Supplementary information

High strength anhydrite cement based on lime mud from water treatment process: one step synthesis in water environment, characterization and technological parameters

Maksim Kamarou 1, Hongbin Tan 2, Dmitry Moskovskikh 3, Xiaoling Ma 4, Feihua Yang 5, Evgenii Beletskii 6, Elena Alekseeva 6, Sergey Yudin 7, Valentin Romanovski 8,*

1 International Information and Analytical Center for Technology Transfer, Belarusian State Technological University. 220006, Sverdlova st., 13a, Minsk, Belarus

2 School of Materials and Chemistry, Southwest University of Science and Technology, Mianyang 621010, China

3 Science and Research Centre of Functional Nano-Ceramics, National University of Science and Technology “MISIS”, 119049, Lenin av., 4, Moscow, Russia

4 School of Materials and Chemistry, Southwest University of Science and Technology, Mianyang 621010, China

5 State Key Laboratory of Solid Waste Resource Utilization and Energy Saving Building Materials, Beijing 100041, China

6 Institute of Chemistry, Saint Petersburg State University, 199034, Universitetskaya embankment, 7-9, St. Petersburg, Russia

7 Research Laboratory of Scanning Probe Microscopy, Moscow Polytechnic University, 38, B. Semenovskaya St, Moscow, Russia

8 Department of Materials Science and Engineering, University of Virginia, Charlottesville, VA 22904, USA

*Correspondence to: Valentin Romanovski, e-mail: vramano@kth.se, phone: +14342829763

Supplementary information includes: additional text

S.1 Materials and reagents

Lime-mud in an air-dry state is lumps with sizes up to several centimeters, the chemical composition is: Ca(OH)2 – 22.2 wt.%, CaCO3 – 61.1 wt.%, CaO – 13 wt.% and a moisture content of 3.7 wt.%, the rest is impurity substances (MgO, SiO2 and other substances added to the lime with carbonate raw materials).

Portland cement brand PC500D0 is Portland cement without mineral additives, produced on the basis of clinker of a standardized mineralogical composition with a limited content of tricalcium aluminate, produced by the Belarusian Cement Company. Chemical composition of Portland cement brand PC500D0, wt.%: SiO2 – 20.5; Al2O3 – 4.1; CaO – 64.9; Fe2O3 – 3.5; MgO – 1.1; TiO2 – 0.2; P2O5 – 0.2; SO3 – 3.1; Na2O – 0.2; K2O – 0.8; Na2Oeq. – 0.7; loss after ignition – 0.9; Cl – 0.01. Mineralogical composition of clinker used to produce Portland cement grade PC500D0, wt.%: C3S – 74.0; C2S – 8.6; C3A – 4.0; C4AF – 11.8; CaOb. – 0.7.

Ca(OH)2 grade “chemically pure” is a white powder with a main component content of more than 99 wt.%, a density of 2.24 g/mL at 25 °C and a solubility of 1.65 g/L (20 °C) in water.

K2SO4 of the “chemically pure” grade is a crystalline substance or powder, white, odorless, with a bitter-salty taste. Easily dissolves in water without undergoing hydrolysis. Insoluble in pure ethyl alcohol, acetone and concentrated alkali solution. Slightly soluble in glycerin. Density – 2.66 g/cm³, content of the main component is not less than 99 wt.%.

S.2 Samples characterization

Normal density measurement. When mixing the binder with water, a dough is formed, the standard consistency of which (the normal thickness of gypsum dough) is determined by the diameter of the dough spread when exiting the cylinder, raised by 180 mm. All characteristics of the binder were assessed using the normal density test, which made it possible to compare them with the requirements of the standard. Considering that normal density depends on the degree of grinding of the binder, its composition and the type of additives included, the study used gypsum binders with the same particle size distribution determined using sieve analysis.

Setting time measurement. To measure the setting time, dough of normal density was used, carried out using a Vick device, in which the needle replaced the pestle at the end of the rod, while the mass of the moving part remained constant and equal to 300 ± 2 g. The dough was prepared from 400 g of binder and an appropriate volume of water, ensuring normal dough density. The initial moment of setting was considered to be the time from the moment the dough began to be mixed (the moment of water flowing out), and the final moment was the moment when the needle stopped lowering 1–1.5 mm to the surface of the plate.

Compressive strength. Binder strength refers to the strength of the stone-like material obtained by mixing gypsum binder with water to create a dough of normal thickness. The compressive strength of samples measuring 20×20×20 mm was measured on a universal testing machine “Instron 1195”, which meets the requirements of GOST 1497-84. The range of load changes was 0–10 kN, and the loading rate of the sample until failure ranged from 0.5–1 mm/min. The breaking force was measured with an accuracy of ±1% using a scale.

The particle size distribution was determined using a Fritsch Particle Sizer Analysette 22 (Germany) in distilled water with an ethanol suspension.

The morphology and elemental composition of the surface of the samples were studied by synthetic gypsum samples using scanning electron microscopy (SEM) methods on a JSM-5610 LV scanning electron microscope equipped with EDXJED-2201 chemical analysis systems (JEOL, Japan).

The phase composition of the synthesized solid phase was carried out on a D8 ADVANCE X-ray diffractometer from the company "Bruker" (Germany). For identification, data from the international Join Committee on Powder Diffraction Standards 2003 file, as well as DIFFRACPLUS software from Bruker, were used. X-ray diffraction patterns were processed using WinPlotr software included in the FullProfSuite package.

Thermogravimetric analysis (TGA) and differential scanning calorimetry (DSC) were carried out on a DTA NETZSCH STA 409 PC/PG instrument (Germany). Approximately 50 mg of sample was placed in a corundum crucible and heated from ambient temperature to 900 °C at a rate of 5 °C/min under a nitrogen flow (100 ml/min). The temperature measurement accuracy was 0.01 °C, and the enthalpy calculation accuracy was 0.01 J/g.

Determination of compressive strength of anhydrite binders. Studies were carried out to establish compressive strength values at the age of 2 hours and 7 days for samples obtained at various pressing pressures of 0.8–1.4 MPa and a holding time of 30 minutes 60 minutes.