The Supplemental Information for “The ‘Overlooked’ Entropy and the Associated Role of Phonons in the Mixing Stabilization for Complex Ceramics”

A. The analytic analyses of the vibrational entropy

For an N-atom lattice, there are 3N vibrational modes with frequencies ωi (i=1,⋯,3N). The vibrational entropy is:

|  | Svib=kBiℏωikBT1expℏωikBT-1-ln1-exp-ℏωikBT | (A1) |
| --- | --- | --- |

Setting Θi=ℏωikB, the sum in Eq. (A1) can be written as a sum of the product of a continuous function f(Θ,T) with delta functions, i.e.:

|  | Svib=kBif(Θ,T)δΘ-Θi, | (A2) |
| --- | --- | --- |
|  | fΘ,T=ΘTexpΘT-1-ln1-exp-ΘT. | (A3) |

There are two terms in fΘ,T which are f1Θ,T=ΘTexpΘT-1 and f2Θ,T=ln1-exp-ΘT. Both f1Θ,T and f2Θ,T are increasing functions of T for a given Θ, while both functions are decreasing function of Θ for a given T.

In the transition metal carbides and diborides, the acoustic modes range between 0-12 THz, which corresponds to values of 0-92 K for Θ. Therefore, curves with Θ=10, 30, 60, 90 K (ω=1.31, 3.93, 7.86, 11.8 THz) are shown in Figure A1. These results suggest that f2Θ,T has much more significant contribution to the vibrational entropy because f1Θ,T is bounded between 0 and 1 while f2Θ,T can quickly exceed this value. Furthermore, f1Θ,T asymptotes to one as the temperature rises, which suggests that only f2Θ,T contributes the change in Svib at high temperatures.

Figure A1 (a) The curves of f1Θ,T=ΘTexpΘT-1 where the black line represent Θ=10 K, blue dashed line for Θ=30 K, red dotted line for Θ=30 K, and green dash-dotted line for Θ=90 K. (b) The curves of f2Θ,T=ln1-exp-ΘT. (c) The curves of ∂f(Θ,T)∂T.

The derivatives of fΘ,T with respect to temperature determine how quickly the vibrational entropy rises, which can be computed as the following:

|  | ∂fΘ,T∂T=Θ24T3csch2Θ2T, | (A4) |
| --- | --- | --- |
|  | ∂fΘ,T∂T≈1T T>Θ, limT→0∂fΘ,T∂T=limT→∞∂fΘ,T∂T=0. | (A5) |

As illustrated in Figure A1(c), the derivatives of ∂fΘ,T∂T exponentially increase from zero to the maximum value and then decrease as 1T after this peak. For the low-frequency vibrational modes, the maximum value of ∂fΘ,T∂T is much larger than that for the high-frequency vibrational modes. Therefore, the low-frequency vibrational modes result in not only large values of Svib but the quick rise in Svib.

B. The special quasi-random structures (SQSs)

The metals form a face-centered-cubic sublattice in B1-structured transition metal carbides and a hexagonal sublattice in the AlB2 prototype transition metal diborides. Therefore, 16-atom supercells of SQSs are generated for the metal sublattice with two elements at different compositions. The lattice vectors (a1,a2,a3) are written in their Cartesian components with the given scaling factor. The ion (atom) positions are provided in the direct coordinates of (a1,a2,a3).

| Mi34Mj14C |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Lattice vectors |  |  |  | a1 | -1 | 1 | 2 |
| a2 | -1 | 2 | 1 | a3 | -2 | 1 | 1 |
| Ion positions |  |  |  |  |  |  |  |
| Mi | 3/8 | 7/8 | 7/8 | C | 3/4 | 3/4 | 3/4 |
| Mi | 3/8 | 3/8 | 7/8 | C | 3/4 | 1/4 | 3/4 |
| Mi | 7/8 | 7/8 | 7/8 | C | 1/4 | 3/4 | 3/4 |
| Mi | 7/8 | 3/8 | 7/8 | C | 1/4 | 1/4 | 3/4 |
| Mi | 1/8 | 5/8 | 5/8 | C | 1/2 | 1/2 | 1/2 |
| Mi | 3/8 | 7/8 | 3/8 | C | 3/4 | 3/4 | 1/4 |
| Mi | 1/8 | 1/8 | 5/8 | C | 1/2 | 1 | 1/2 |
| Mi | 3/8 | 3/8 | 3/8 | C | 3/4 | 1/4 | 1/4 |
| Mi | 5/8 | 5/8 | 5/8 | C | 1 | 1/2 | 1/2 |
| Mi | 7/8 | 7/8 | 3/8 | C | 1/4 | 3/4 | 1/4 |
| Mi | 7/8 | 3/8 | 3/8 | C | 1 | 1 | 1/2 |
| Mi | 1/8 | 5/8 | 1/8 | C | 1/4 | 1/4 | 1/4 |
| Mj | 5/8 | 1/8 | 5/8 | C | 1/2 | 1/2 | 1 |
| Mj | 1/8 | 1/8 | 1/8 | C | 1/2 | 1 | 1 |
| Mj | 5/8 | 5/8 | 1/8 | C | 1 | 1/2 | 1 |
| Mj | 5/8 | 1/8 | 1/8 | C | 1 | 1 | 1 |

| Mi12Mj12C |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Lattice vectors |  |  |  | a1 | -1 | 1 | 2 |
| a2 | -1 | 2 | 1 | a3 | -2 | 1 | 1 |
| Ion positions |  |  |  |  |  |  |  |
| Mi | 3/8 | 7/8 | 7/8 | C | 3/4 | 3/4 | 3/4 |
| Mi | 1/8 | 5/8 | 5/8 | C | 3/4 | 1/4 | 3/4 |
| Mi | 3/8 | 7/8 | 3/8 | C | 1/4 | 3/4 | 3/4 |
| Mi | 3/8 | 3/8 | 3/8 | C | 1/4 | 1/4 | 3/4 |
| Mi | 7/8 | 7/8 | 3/8 | C | 1/2 | 1/2 | 1/2 |
| Mi | 1/8 | 5/8 | 1/8 | C | 3/4 | 3/4 | 1/4 |
| Mi | 1/8 | 1/8 | 1/8 | C | 1/2 | 1 | 1/2 |
| Mi | 5/8 | 5/8 | 1/8 | C | 3/4 | 1/4 | 1/4 |
| Mj | 3/8 | 3/8 | 7/8 | C | 1 | 1/2 | 1/2 |
| Mj | 7/8 | 7/8 | 7/8 | C | 1/4 | 3/4 | 1/4 |
| Mj | 7/8 | 3/8 | 7/8 | C | 1 | 1 | 1/2 |
| Mj | 1/8 | 1/8 | 5/8 | C | 1/4 | 1/4 | 1/4 |
| Mj | 5/8 | 5/8 | 5/8 | C | 1/2 | 1/2 | 1 |
| Mj | 5/8 | 1/8 | 5/8 | C | 1/2 | 1 | 1 |
| Mj | 7/8 | 3/8 | 3/8 | C | 1 | 1/2 | 1 |
| Mj | 5/8 | 1/8 | 1/8 | C | 1 | 1 | 1 |

| Mi78Mj18B2 |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Lattice vectors |  |  |  | a1 | -2 | 0 | 2.2 |
| a2 | -2 | 0 | 2.2 | a3 | 1 | -3 | -2.2 |
| Ion positions |  |  |  |  |  |  |  |
| Mi | 1 | 1 | 1/2 | B | 5/24 | 3/8 | 5/6 |
| Mi | 1 | 1/2 | 1/2 | B | 11/24 | 1/8 | 5/6 |
| Mi | 1/4 | 1/4 | 1/2 | B | 17/24 | 7/8 | 5/6 |
| Mi | 1/2 | 1 | 1/2 | B | 23/24 | 5/8 | 1/3 |
| Mi | 1 | 1 | 1 | B | 11/24 | 5/8 | 5/6 |
| Mi | 1/4 | 3/4 | 1/2 | B | 17/24 | 3/8 | 5/6 |
| Mi | 1/2 | 1/2 | 1/2 | B | 23/24 | 1/8 | 5/6 |
| Mi | 3/4 | 1/4 | 1/2 | B | 23/24 | 5/8 | 5/6 |
| Mi | 1 | 1/2 | 1 | B | 1/24 | 7/8 | 1/6 |
| Mi | 3/4 | 3/4 | 1/2 | B | 1/24 | 3/8 | 1/6 |
| Mi | 1/4 | 3/4 | 1 | B | 7/24 | 1/8 | 1/6 |
| Mi | 1/2 | 1/2 | 1 | B | 13/24 | 7/8 | 1/6 |
| Mi | 3/4 | 1/4 | 1 | B | 1/24 | 7/8 | 2/3 |
| Mi | 3/4 | 3/4 | 1 | B | 7/24 | 5/8 | 1/6 |
| Mj | 1/4 | 1/4 | 1 | B | 13/24 | 3/8 | 1/6 |
| Mj | 1/2 | 1 | 1 | B | 19/24 | 1/8 | 1/6 |
| B | 5/24 | 7/8 | 1/3 | B | 1/24 | 3/8 | 2/3 |
| B | 5/24 | 3/8 | 1/3 | B | 7/24 | 1/8 | 2/3 |
| B | 11/24 | 1/8 | 1/3 | B | 13/24 | 7/8 | 2/3 |
| B | 17/24 | 7/8 | 1/3 | B | 19/24 | 5/8 | 1/6 |
| B | 5/24 | 7/8 | 5/6 | B | 7/24 | 5/8 | 2/3 |
| B | 11/24 | 5/8 | 1/3 | B | 13/24 | 3/8 | 2/3 |
| B | 17/24 | 3/8 | 1/3 | B | 19/24 | 1/8 | 2/3 |
| B | 23/24 | 1/8 | 1/3 | B | 19/24 | 5/8 | 2/3 |

| Mi34Mj14B2 |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Lattice vectors |  |  |  | a1 | -1 | 3 | 2.2 |
| a2 | -1 | 3 | -2.2 | a3 | -32 | -32 | 0 |
| Ion positions |  |  |  |  |  |  |  |
| Mi | 1/8 | 5/8 | 1/2 | B | 3/4 | 1/2 | 1/6 |
| Mi | 1 | 1/2 | 1 | B | 5/8 | 3/8 | 2/3 |
| Mi | 3/8 | 7/8 | 1/2 | B | 1 | 3/4 | 1/6 |
| Mi | 1/4 | 3/4 | 1 | B | 7/8 | 5/8 | 2/3 |
| Mi | 1/8 | 1/8 | 1/2 | B | 3/4 | 1 | 1/6 |
| Mi | 1 | 1 | 1 | B | 5/8 | 7/8 | 2/3 |
| Mi | 3/8 | 3/8 | 1/2 | B | 1 | 1/4 | 1/6 |
| Mi | 1/4 | 1/4 | 1 | B | 7/8 | 1/8 | 2/3 |
| Mi | 1/2 | 1/2 | 1 | B | 3/8 | 5/8 | 1/3 |
| Mi | 3/4 | 3/4 | 1 | B | 1/4 | 1/2 | 5/6 |
| Mi | 1/2 | 1 | 1 | B | 5/8 | 7/8 | 1/3 |
| Mi | 7/8 | 3/8 | 1/2 | B | 1/2 | 3/4 | 5/6 |
| Mj | 5/8 | 5/8 | 1/2 | B | 3/8 | 1/8 | 1/3 |
| Mj | 7/8 | 7/8 | 1/2 | B | 1/4 | 1 | 5/6 |
| Mj | 5/8 | 1/8 | 1/2 | B | 5/8 | 3/8 | 1/3 |
| Mj | 3/4 | 1/4 | 1 | B | 1/2 | 1/4 | 5/6 |
| B | 1/4 | 1/2 | 1/6 | B | 7/8 | 5/8 | 1/3 |
| B | 1/8 | 3/8 | 2/3 | B | 3/4 | 1/2 | 5/6 |
| B | 1/2 | 3/4 | 1/6 | B | 1/8 | 7/8 | 1/3 |
| B | 3/8 | 5/8 | 2/3 | B | 1 | 3/4 | 5/6 |
| B | 1/4 | 1 | 1/6 | B | 7/8 | 1/8 | 1/3 |
| B | 1/8 | 7/8 | 2/3 | B | 3/4 | 1 | 5/6 |
| B | 1/2 | 1/4 | 1/6 | B | 1/8 | 3/8 | 1/3 |
| B | 3/8 | 1/8 | 2/3 | B | 1 | 1/4 | 5/6 |

| Mi58Mj38B2 |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Lattice vectors |  |  |  | a1 | -2 | 0 | 2.2 |
| a2 | -2 | 0 | 2.2 | a3 | 1 | -3 | -2.2 |
| Ion positions |  |  |  |  |  |  |  |
| Mi | 1 | 1 | 1/2 | B | 5/24 | 3/8 | 5/6 |
| Mi | 1 | 1/2 | 1/2 | B | 11/24 | 1/8 | 5/6 |
| Mi | 1/4 | 1/4 | 1/2 | B | 17/24 | 7/8 | 5/6 |
| Mi | 1/2 | 1 | 1/2 | B | 23/24 | 5/8 | 1/3 |
| Mi | 1/4 | 3/4 | 1/2 | B | 11/24 | 5/8 | 5/6 |
| Mi | 1/2 | 1/2 | 1/2 | B | 17/24 | 3/8 | 5/6 |
| Mi | 1/4 | 1/4 | 1 | B | 23/24 | 1/8 | 5/6 |
| Mi | 1/2 | 1 | 1 | B | 23/24 | 5/8 | 5/6 |
| Mi | 1/2 | 1/2 | 1 | B | 1/24 | 7/8 | 1/6 |
| Mi | 3/4 | 1/4 | 1 | B | 1/24 | 3/8 | 1/6 |
| Mj | 1 | 1 | 1 | B | 7/24 | 1/8 | 1/6 |
| Mj | 3/4 | 1/4 | 1/2 | B | 13/24 | 7/8 | 1/6 |
| Mj | 1 | 1/2 | 1 | B | 1/24 | 7/8 | 2/3 |
| Mj | 3/4 | 3/4 | 1/2 | B | 7/24 | 5/8 | 1/6 |
| Mj | 1/4 | 3/4 | 1 | B | 13/24 | 3/8 | 1/6 |
| Mj | 3/4 | 3/4 | 1 | B | 19/24 | 1/8 | 1/6 |
| B | 5/24 | 7/8 | 1/3 | B | 1/24 | 3/8 | 2/3 |
| B | 5/24 | 3/8 | 1/3 | B | 7/24 | 1/8 | 2/3 |
| B | 11/24 | 1/8 | 1/3 | B | 13/24 | 7/8 | 2/3 |
| B | 17/24 | 7/8 | 1/3 | B | 19/24 | 5/8 | 1/6 |
| B | 5/24 | 7/8 | 5/6 | B | 7/24 | 5/8 | 2/3 |
| B | 11/24 | 5/8 | 1/3 | B | 13/24 | 3/8 | 2/3 |
| B | 17/24 | 3/8 | 1/3 | B | 19/24 | 1/8 | 2/3 |
| B | 23/24 | 1/8 | 1/3 | B | 19/24 | 5/8 | 2/3 |

| Mi12Mj12B2 |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Lattice vectors |  |  |  | a1 | -2 | 0 | 2.2 |
| a2 | -2 | 0 | 2.2 | a3 | 1 | -3 | -2.2 |
| Ion positions |  |  |  |  |  |  |  |
| Mi | 1 | 1 | 1/2 | B | 5/24 | 3/8 | 5/6 |
| Mi | 1 | 1/2 | 1/2 | B | 11/24 | 1/8 | 5/6 |
| Mi | 1/4 | 1/4 | 1/2 | B | 17/24 | 7/8 | 5/6 |
| Mi | 1/4 | 3/4 | 1/2 | B | 23/24 | 5/8 | 1/3 |
| Mi | 1 | 1/2 | 1 | B | 11/24 | 5/8 | 5/6 |
| Mi | 1/4 | 1/4 | 1 | B | 17/24 | 3/8 | 5/6 |
| Mi | 1/2 | 1/2 | 1 | B | 23/24 | 1/8 | 5/6 |
| Mi | 3/4 | 1/4 | 1 | B | 23/24 | 5/8 | 5/6 |
| Mj | 1/2 | 1 | 1/2 | B | 1/24 | 7/8 | 1/6 |
| Mj | 1 | 1 | 1 | B | 1/24 | 3/8 | 1/6 |
| Mj | 1/2 | 1/2 | 1/2 | B | 7/24 | 1/8 | 1/6 |
| Mj | 3/4 | 1/4 | 1/2 | B | 13/24 | 7/8 | 1/6 |
| Mj | 1/2 | 1 | 1 | B | 1/24 | 7/8 | 2/3 |
| Mj | 3/4 | 3/4 | 1/2 | B | 7/24 | 5/8 | 1/6 |
| Mj | 1/4 | 3/4 | 1 | B | 13/24 | 3/8 | 1/6 |
| Mj | 3/4 | 3/4 | 1 | B | 19/24 | 1/8 | 1/6 |
| B | 5/24 | 7/8 | 1/3 | B | 1/24 | 3/8 | 2/3 |
| B | 5/24 | 3/8 | 1/3 | B | 7/24 | 1/8 | 2/3 |
| B | 11/24 | 1/8 | 1/3 | B | 13/24 | 7/8 | 2/3 |
| B | 17/24 | 7/8 | 1/3 | B | 19/24 | 5/8 | 1/6 |
| B | 5/24 | 7/8 | 5/6 | B | 7/24 | 5/8 | 2/3 |
| B | 11/24 | 5/8 | 1/3 | B | 13/24 | 3/8 | 2/3 |
| B | 17/24 | 3/8 | 1/3 | B | 19/24 | 1/8 | 2/3 |
| B | 23/24 | 1/8 | 1/3 | B | 19/24 | 5/8 | 2/3 |