Layered-Columnar Cathode Materials for Sodium-Ion Batteries

Xiaolin Zhaoa,b, Yi Lia,b, Youwei Wanga,b, Erhong Songa,b, Ruguang Mad,*, Jianjun Liua,b,c*

aState Key Laboratory of High Performance Ceramics and Superfine Microstructure, Shanghai Institute of Ceramics, Chinese Academy of Sciences, 1295 Dingxi Road, Shanghai 200050, China

bCenter of Materials Science and Optoelectronics Engineering, University of Chinese Academy of Sciences, Beijing 100049, China

cSchool of Chemistry and Materials Science, Hangzhou Institute for Advanced Study, University of Chinese Academy of Sciences, 1 Sub-lane Xiangshan, Hangzhou 310024, China

dSchool of Materials Science and Engineering, Suzhou University of Science and Technology, 99 Xuefu Road Suzhou, 215011, China.

Corresponding Author

* E-mail Address: ruguangma@usts.edu.cn, jliu@mail.sic.ac.cn

Methods

Synthesis of NaFe[O3PCH(OH)CO2]. A mixture of FeSO4·7H2O (0.278 g, 1.0 mmol), NH4Cl (4.86 g, 90 mmol), NaF (0.798 g, 19 mmol), CH(OH)(CO2H)(PO3H2) solution (1.4 mL, 2.0 mmol), and H2O (20.0 mL) was stirred, then transferred to a 50-mL Teflon-lined stainless-steel autoclave and heated at 150°C for 96 h. The final mixture was repeatedly rinsed with distilled water under ultrasonic treatment and dried at 70°C for 24 hours to obtain pure colorless crystals.

Synthesis of maricite NaFePO4. Fe(NO3)3·9H2O (1.616 g, 4 mmol), (NH4)2HPO4 (0.46 g, 4 mmol), NaOH (0.16 g, 4 mmol), citric acid (1.26, 6.0 mmol), and H2O (60.0 mL) was mixed homogeneously in a beaker, then the pH of the mixed solution was adjusted to be about 7 with ammonia. Further, the beaker was placed in a constant temperature oil bath at 80 ℃ and the mixed solution was stirred to a transparent sol. Subsequently, the transparent sol was vacuum dried at 60 ℃ for 12 h, then calcined at 350 ℃ for 3 h and continued to raise the temperature to 700 ℃ for 10 h in N2 atmosphere.

Electrochemical measurements. The active materials NaFe[O3PCH(OH)CO2] were ball-milled with Super P (weight ratio of 7.5:2.5) at a speed of 400 rpm for 12 hours. The obtained mixture was then mixed with Super P and polyvinylidene fluoride (PVDF) binder that to dissolve in N-methyl-2-pyrrolidone (NMP) solution at a weight ratio of 8:1:1, then evenly coated on the Al plate and dried in a vacuum oven at 100 °C for 12 h. The CR2032 coin cells were assembled in an argon-filled glovebox where the content of O2 and H2O was less than 0.1 ppm. The cells were composed of Na anodes, NaFe[O3PCH(OH)CO2] cathodes, Waterman GF/C glass fiber separators and 150 μl cm-2 electrolyte (1 mol/L NaClO4 in a 1:1 mixture of ethylene carbonate (EC) and dimethyl carbonate (DMC) with 5.0% FEC). Galvanostatic discharge-charge tests were performed at 25 ℃ using LAND electrochemical testing system. Cyclic voltammetry (CV) measurements were carried out on Bio-logic VSP between 1.5 V and 4.2 V at a scan rate of 0.5 mV s-1. The preparation conditions and testing environment of NaFePO4 cathode materials were identical to those of NaFe[O3PCH(OH)CO2].

Characterizations. The crystal structures of materials were examined by powder X-ray diffraction (XRD, Bruker D8 Advance) using Cu Kα radiation between 10° and 60° with a scan speed of 2° min−1. For in situ XRD experiments we have developed our own 35 mm inner diameter electrochemical cell, equipped with a Be window as a current collector, operating in reflection geometry. The in-situ cell was charged/discharged at a rate of 0.2 C with a sampling interval of 30 minutes for X-ray collection. The morphology of the samples was investigated by scanning electron microscope (SEM, FEI Verios G4). The elemental distribution was characterized by energy dispersive spectrograms (EDS). The cells after discharging and charging were disassembled in argon-filled glove box, the samples were washed by 1,2-dimethoxyethane (DME) for 0.5 h and then dried for 2 h under vacuum to remove the residual solvent. The valence states of the samples were investigated with X-ray photoelectron spectroscopy (XPS, Escalab 250). The Fourier transform infrared spectroscopy (FTIR) measurements were implemented on a Nicolet 6700 spectrometer (Thermo) in the range 4000-750 cm-1.

Density functional theory calculations. The first-principles calculations were conducted within the formalism of spin-polarization density functional theory (DFT) and the generalized gradient approximation (GGA) of the exchange-correlation function as formulated by Perdew, Burke, and Ernzerhof1. The valence electron−ion interaction was treated by the projector augmented wave (PAW) potential2 in the Vienna Ab initio Simulation Package (VASP)3-4.The van der Waals-augmented density functional theory (vdW-DFT) was used to modify exchange and correlation energies5. For the organic materials, the function of DFT is limited because of the proverbially poor ability to depict the long-range van der Waals (vdW) interaction between the molecules6. So the empirical dispersions of Grimme (DFT-D2) was applied to account for the long-range vdW interactions7. The DFT+U approach has been successfully applied in systems with strongly correlated d and f electrons. The Ueff values of 3.9 for Fe are taken.

The wave functions were expanded in plane-wave basis set up to a kinetic energy cutoff of 520 eV. Brillouin-zone integrations were performed by using the k-point sampling of the Monkhorst-Pack scheme with a 2×2×2 grid8. The convergence of total energy with respect to the kinetic energy cutoff and the k-point sampling has been carefully examined. The convergence criterion of energy and structural relaxation were set as less than 1.0×10-5 eV and 0.01 eV/Å, respectively. Minimization of the total energy was realized with a full relaxation of the atomic positions and cell parameters for each structure.

The phonon dispersion calculations were performed by using the Parlinski–Li–Kawazoe methodology implemented in the PHONOPY code9, based on the Hellmann–Feynman forces calculated with the VASP code. The force constants are determined from the Hellmann–Feynman forces induced by the displacement of an atom in a sufficiently large supercell (2×2×2). The phonon frequencies and polarization vectors are then obtained by diagonalizing the dynamical matrices. In this work, the atomic displacements are set to 0.01 Å. The minimum energy path (MEP) for Na-ions migration is obtained from the climbing image nudged elastic band (CINEB)10 method with a force convergence tolerance of 0.01 eV Å-1. The BVSE calculations were performed using the SoftBV code11 and the visualization of isosurfaces was carried out using VESTA software12.

Figure S1. The XPS of NaFe[O3PCH(OH)CO2].

Figure S2. The XRD of maricite NaFePO4

Figure S3. Galvanostatic charge-discharge curves of maricite NaFePO4 at 0.1C (1C=120 mAh g-1).

Figure S4. Cycling performance of maricite NaFePO4 at 2C for 400 cycles.

Table S1. The comparison of ACTP (Actual Capacity (CA) to Theoretical Capacity (CT) Percentage) between our work and reported cathode materials for sodium ions batteries.

|  | Cathode Material | Theoretical Capacity (CT) | Actual Capacity (CA) | ACTP |
| --- | --- | --- | --- | --- |
| Layered Transition Metal Oxides | Ca0.07Na0.26MnO213 | 70.5 | 40.0 | 56.7% |
|  | Na0.4MnO213 | 111.3 | 38 | 34.1% |
|  | Na2/3[Ni1/3Mn2/3]O214 | 172.5 | 150 | 86.9% |
|  | Na2/3[Mg0.28Mn0.72]O215 | 190.7 | 162.5 | 85.2% |
|  | Na0.5Ni0.22Co0.11Mn0.66O216 | 135 | 98.8 | 73.2% |
|  | Na2/3Li1/6Fe1/6Co1/6Ni1/6Mn1/3O217 | 186.8 | 160.5 | 85.9% |
|  | O3-Na3Ni2BiO618 | 163.6 | 97 | 59.2% |
|  | Na0.7Ni0.35Sn0.65O219 | 128 | 64 | 50% |
|  | P2-Na0.78Co1/2Mn1/3Ni1/6O220 | 194.3 | 129 | 66.3% |
| Metal-Organic Framework Materials | Na2Fe(C2O4)SO4 ·H2O21 | 176 | 75 | 42.6% |
|  | Na2Fe(C2O4)(HPO4)22 | 187.2 | 104 | 55.6% |
|  | Na2Fe(C2O4)F223 | 248 | 69.4 | 56% |
|  | NaFe[O3PCH(OH)CO2] | 113.6 | 106.1 | 93.4% |
| Polyanionic Compounds | Na3(VOPO4)2F24 | 195 | 130 | 66.7% |
|  | Na4MnCr(PO4)325 | 221.3 | 108.4 | 48.9% |
|  | Na3V2(PO4)2F326 | 192 | 128 | 66.7% |
|  | Na3V1.9(Ca,Mg,Al,Cr,Mn)0.1(PO4)2F327 | 192 | 118.5 | 61.7% |
|  | Na3MnPO4CO328 | 240 | 97 | 40.4% |
|  | Na3FePO4CO329 | 248.8 | 113 | 45.4% |
|  | NaFePO430 | 155 | 104.9 | 67.6% |
|  | NASICON-typeNa4Fe3(PO4)2(P2O7)/C31 | 129 | 113.0 | 87.6% |
| Prussian Blue Analogues | Na1.73K0.13MnFe(CN)6 | 148.7 | 136.6 | 91.8% |
|  | Na1.72MnFe(CN)6 | 150.3 | 121 | 80.5% |
| Organic Sodium Slat | Na2AQ26DS32 | 130 | 119 | 91.5% |
|  | Na4C8H2O633 | 223 | 184 | 89% |

Figure S5. Ex-situ XRD analysis of NaFe[O3PCH(OH)CO2] cathode during different charging and discharging process.

Figure S6. The electrostatic energies of Na1-xFe[O3PCH(OH)CO2] (x=1/8, 2/8, ···, 7/8, 8/8) crystal structures were screened by Supercell software.

Figure S7. The Na-ions de-intercalation sites and the structural evolution of Na1xFe[O3PCH(OH)CO2] (x=1/8, 3/8, 5/8, 7/8)

Figure S8. The crystal structure of NaFe[O3PCH(OH)CO2] along a-axis direction and c-axis direction.

Figure S9. Changes in Fe-O bond lengths in the [FeO6] octahedron during the de-embedding of sodium ions from the NaFe[O3PCH(OH)CO2] structure.

Figure S10. The bottleneck size of Na-ions passing through between (a) two co-side polyhedrons (Na1→Na1), (b) Na1→Na2

Figure S11. a. The olivine structure of NaFePO4 and the activation energy of sodium ions migration in the ab plane. b. The maricite structure of NaFePO4 and activation energy of sodium ions migration along the c-axis direction.

References

1.	Perdew, J. P.; Burke, K.; Ernzerhof, M., Generalized gradient approximation made simple. Phys. Rev. Lett. 1996, 77 (18), 3865-3868.

2.	Perdew, J. P.; Chevary, J. A.; Vosko, S. H.; Jackson, K. A.; Pederson, M. R.; Singh, D. J.; Fiolhais, C., Atoms, molecules, solids, and surfaces: Applications of the generalized gradient approximation for exchange and correlation. Phys. Rev. B 1992, 46 (11), 6671-6687.

3.	Kresse, G.; Furthmuller, J., Efficiency of ab-initio total energy calculations for metals and semiconductors using a plane-wave basis set. Comput. Mater. Sci. 1996, 6 (1), 15-50.

4.	Kresse, G.; Furthmuller, J., Efficient iterative schemes for ab initio total-energy calculations using a plane-wave basis set. Phys. Rev. B 1996, 54 (16), 11169-11186.

5.	Savasta, S.; Di Stefano, O.; Savona, V.; Langbein, W., Quantum complementarity of microcavity polaritons. Phys. Rev. Lett. 2005, 94 (24), 246401.

6.	Hobza, P.; Sponer, J.; Reschel, T., Density-Functional Theory and Molecular Clusters. J. Comput. Chem. 1995, 16 (11), 1315-1325.

7.	Grimme, S., Semiempirical GGA-type density functional constructed with a long-range dispersion correction. J. Comput. Chem. 2006, 27 (15), 1787-1799.

8.	Monkhorst, H. J.; Pack, J. D., Special points for Brillouin-zone integrations. Phys. Rev. B 1976, 13 (12), 5188-5192.

9.	Togo, A.; Tanaka, I., First principles phonon calculations in materials science. Scr. Mater. 2015, 108, 1-5.

10. Henkelman, G.; Uberuaga, B. P.; Jonsson, H., A climbing image nudged elastic band method for finding saddle points and minimum energy paths. J. Chem. Phys. 2000, 113 (22), 9901-9904.

11. Chen, H.; Wong, L. L.; Adams, S., SoftBV - a software tool for screening the materials genome of inorganic fast ion conductors. Acta Crystallogr B Struct Sci Cryst Eng Mater 2019, 75 (Pt 1), 18-33.

12. Momma, K.; Izumi, F., VESTA: a three-dimensional visualization system for electronic and structural analysis. J. Appl. Crystallogr. 2008, 41 (3), 653-658.

13. Chae, M. S.; Chakraborty, A.; Kunnikuruvan, S.; Attias, R.; Maddukuri, S.; Gofer, Y.; Major, D. T.; Aurbach, D., Vacancy-Driven High Rate Capabilities in Calcium-Doped Na0.4MnO2 Cathodes for Aqueous Sodium-Ion Batteries. Adv. Energy Mater. 2020, 10 (37), 2002077.

14.	 Somerville, J. W.; Sobkowiak, A.; Tapia-Ruiz, N.; Billaud, J.; Lozano, J. G.; House, R. A.; Gallington, L. C.; Ericsson, T.; Häggström, L.; Roberts, M. R.; Maitra, U.; Bruce, P. G., Nature of the “Z”-phase in layered Na-ion battery cathodes. Energy Environ. Sci. 2019, 12 (7), 2223-2232.

15. Maitra, U.; House, R. A.; Somerville, J. W.; Tapia-Ruiz, N.; Lozano, J. G.; Guerrini, N.; Hao, R.; Luo, K.; Jin, L.; Perez-Osorio, M. A.; Massel, F.; Pickup, D. M.; Ramos, S.; Lu, X.; McNally, D. E.; Chadwick, A. V.; Giustino, F.; Schmitt, T.; Duda, L. C.; Roberts, M. R.; Bruce, P. G., Oxygen redox chemistry without excess alkali-metal ions in Na2/3[Mg0.28Mn0.72]O2. Nat. Chem. 2018, 10 (3), 288-295.

16.	 Chagas, L. G.; Buchholz, D.; Vaalma, C.; Wu, L.; Passerini, S., P-type NaxNi0.22Co0.11Mn0.66O2materials: linking synthesis with structure and electrochemical performance. J. Mater. Chem. A 2014, 2 (47), 20263-20270.

17.	 Yao, L.; Zou, P.; Wang, C.; Jiang, J.; Ma, L.; Tan, S.; Beyer, K. A.; Xu, F.; Hu, E.; Xin, H. L., High‐Entropy and Superstructure‐Stabilized Layered Oxide Cathodes for Sodium‐Ion Batteries. Adv. Energy Mater. 2022, 12 (41), 2201989.

18. Zemlyanushin, E.; Pfeifer, K.; Sarapulova, A.; Etter, M.; Ehrenberg, H.; Dsoke, S., Probing the Effect of Titanium Substitution on the Sodium Storage in Na3Ni2BiO6 Honeycomb-Type Structure. Energies 2020, 13 (24), 6498.

19. Wang, P. F.; Xin, H.; Zuo, T. T.; Li, Q.; Yang, X.; Yin, Y. X.; Gao, X.; Yu, X.; Guo, Y. G., An Abnormal 3.7 Volt O3-Type Sodium-Ion Battery Cathode. Angew. Chem. Int. Ed. Engl. 2018, 57 (27), 8178-8183.

20. Hakim, C.; Sabi, N.; Ma, L. A.; Dahbi, M.; Brandell, D.; Edstrom, K.; Duda, L. C.; Saadoune, I.; Younesi, R., Understanding the redox process upon electrochemical cycling of the P2-Na0.78Co1/2Mn1/3Ni1/6O2 electrode material for sodium-ion batteries. Commun. Chem. 2020, 3 (1), 9.

21.	 Song, T.; Yao, W.; Kiadkhunthod, P.; Zheng, Y.; Wu, N.; Zhou, X.; Tunmee, S.; Sattayaporn, S.; Tang, Y., A Low-Cost and Environmentally Friendly Mixed Polyanionic Cathode for Sodium-Ion Storage. Angew. Chem. Int. Ed. Engl. 2020, 59 (2), 740-745.

22.	 Pramanik, A.; Bradford, A. J.; Lee, S. L.; Lightfoot, P.; Armstrong, A. R., Na2Fe(C2O4)(HPO4): a promising new oxalate-phosphate based mixed polyanionic cathode for Li/Na ion batteries. Journal of Physics: Materials 2021, 4 (2), 024004.

23.	 Yao, W.; Sougrati, M.-T.; Hoang, K.; Hui, J.; Lightfoot, P.; Armstrong, A. R., Na2Fe(C2O4)F2: A New Iron-Based Polyoxyanion Cathode for Li/Na Ion Batteries. Chem. Mater. 2017, 29 (5), 2167-2172.

24.	 Shen, X.; Zhou, Q.; Han, M.; Qi, X.; Li, B.; Zhang, Q.; Zhao, J.; Yang, C.; Liu, H.; Hu, Y. S., Rapid mechanochemical synthesis of polyanionic cathode with improved electrochemical performance for Na-ion batteries. Nat. Commun. 2021, 12 (1), 2848.

25.	 Zhang, W.; Li, H.; Zhang, Z.; Xu, M.; Lai, Y.; Chou, S. L., Full Activation of Mn4+/Mn3+ Redox in Na4MnCr(PO4)3 as a High‐Voltage and High‐Rate Cathode Material for Sodium‐Ion Batteries. Small 2020, 16 (25), 2001524.

26.	 Yan, G.; Mariyappan, S.; Rousse, G.; Jacquet, Q.; Deschamps, M.; David, R.; Mirvaux, B.; Freeland, J. W.; Tarascon, J. M., Higher energy and safer sodium ion batteries via an electrochemically made disordered Na3V2(PO4)2F3 material. Nat. Commun. 2019, 10 (1), 585.

27.	 Gu, Z. Y.; Guo, J. Z.; Cao, J. M.; Wang, X. T.; Zhao, X. X.; Zheng, X. Y.; Li, W. H.; Sun, Z. H.; Liang, H. J.; Wu, X. L., An Advanced High-Entropy Fluorophosphate Cathode for Sodium-Ion Batteries with Increased Working Voltage and Energy Density. Adv. Mater. 2022, 34 (14), e2110108.

28.	 Chen, H.; Hao, Q.; Zivkovic, O.; Hautier, G.; Du, L.-S.; Tang, Y.; Hu, Y.-Y.; Ma, X.; Grey, C. P.; Ceder, G., Sidorenkite (Na3MnPO4CO3): A New Intercalation Cathode Material for Na-Ion Batteries. Chem. Mater. 2013, 25 (14), 2777-2786.

29.	 Xie, B.; Sakamoto, R.; Kitajou, A.; Nakamoto, K.; Zhao, L.; Okada, S.; Fujita, Y.; Oka, N.; Nishida, T.; Kobayashi, W.; Okada, M.; Takahara, T., Cathode Properties of Na3FePO4CO3 Prepared by the Mechanical Ball Milling Method for Na-ion Batteries. Sci. Rep. 2020, 10 (1), 3278.

30. Liu, Y.; Zhang, N.; Wang, F.; Liu, X.; Jiao, L.; Fan, L.-Z., Approaching the Downsizing Limit of Maricite NaFePO4 toward High-Performance Cathode for Sodium-Ion Batteries. Adv. Funct. Mater. 2018, 28 (30), 1801917.

31.	 Wu, X.; Zhong, G.; Yang, Y., Sol-gel synthesis of Na4Fe3(PO4)2(P2O7)/C nanocomposite for sodium ion batteries and new insights into microstructural evolution during sodium extraction. J. Power Sources 2016, 327, 666-674.

32. Tang, W.; Liang, R.; Li, D.; Yu, Q.; Hu, J.; Cao, B.; Fan, C., Highly Stable and High Rate-Performance Na-Ion Batteries Using Polyanionic Anthraquinone as the Organic Cathode. ChemSusChem 2019, 12 (10), 2181-2185.

33. Wang, S.; Wang, L.; Zhu, Z.; Hu, Z.; Zhao, Q.; Chen, J., All organic sodium-ion batteries with Na4C8H2O6. Angew. Chem. Int. Ed. Engl. 2014, 53 (23), 5892-5896.