Commercially available snail secretion filtrates: evaluation of extraction methods and functional properties

Maria Francesca Di Filippo1, Luisa Stella Dolci2, Francesca Bonvicini3, Francesca Sparla4, Giovanna Angela Gentilomi3,5, Silvia Panzavolta1*, Nadia Passerini6, Beatrice Albertini6

1Department of Chemistry “G. Ciamician”, University of Bologna, Via Selmi 2, 40126, Bologna, Italy;

2 Department of Industrial Chemistry "Toso Montanari", University of Bologna, Viale del Risorgimento 4,

40136, Bologna, Italy

3Department of Pharmacy and Biotechnology, University of Bologna, Via Massarenti 9, 40138, Bologna, Italy

4Department of Pharmacy and Biotechnology, University of Bologna, Via Irnerio 42, 40138, Bologna, Italy

5 Microbiology Unit, IRCCS Azienda Ospedaliero-Universitaria di Bologna, Via Massarenti 9, 40138, Bologna, Italy

6Department of Pharmacy and Biotechnology, University of Bologna, Via S. Donato 19/2, 40127, Bologna, Italy;

*Corresponding author

silvia.panzavolta@unibo.it

Department of Chemistry G. Ciamician

University of Bologna

Via Selmi 2 40126 Bologna Italy

Phone: +39 051 2099566

Figure S1. Digital image of the brown residue collected from SSF C1, and the relative FT-IR spectrum.

Figure S2. X-Rays diffraction patterns collected on freeze-dried SSFs, before and after dialysis: A as received (red line) and after dialysis (pink); B as received (blue line) and after dialysis (light blue); C1 as received (brown line) and after dialysis (orange); C2 as received (green line) and after dialysis (light green).

Table S1. ICP analysis of dialyzed SSF A

| Element | Wavelength (nm) | Concentration (mg/Kg) | %RSD |
| --- | --- | --- | --- |
| Al | 394.401 | 0.08 | 1.57 |
| P | 214.915 | ND |  |
| Se | 206.275 | ND |  |
| Zn | 213.857 | 0.49 | 0.94 |
| Fe | 371.993 | 0.15 | 0.79 |
| Ca | 616.217 | 13.46 | 0.31 |
| Ba | 553.548 | 0.07 | 1.02 |
| Cu | 324.754 | 0.24 | 0.86 |
| Ni | 341.476 361.939 | ND ND |  |
| K | 769.897 | 6.89 | 0.23 |
| Pb | 405.781 | ND |  |
| Cr | 367.558 425.433 | ND ND |  |
| Mg | 383.829 | 1.05 | 0.52 |
| Mn | 403.449 | 0.005 | 3.05 |
| Na | 589.592 | 4.91 | 0.94 |

ND= Not Detectable

Table S2. ICP analysis of dialyzed SSF B

| Element | Wavelength (nm) | Concentration (mg/Kg) | %RSD |
| --- | --- | --- | --- |
| Al | 394.401 | 0.03 | 1.57 |
| P | 214.915 | ND |  |
| Se | 206.275 | ND |  |
| Zn | 213.857 | 0.72 | 0.51 |
| Fe | 373.486 | 0.16 | 0.13 |
| Ca | 422.673 | 19.38 | 0.28 |
| Ba | 553.548 | 0.06 | 0.77 |
| Cu | 327.395 | 0.24 | 0.55 |
| Ni | 341.476 361.939 | ND ND |  |
| K | 769.897 | 6.00 | 0.85 |
| Pb | 405.781 | ND |  |
| Cr | 367.558 | ND |  |
| Mg | 285.213 | 0.94 | 1.27 |
| Mn | 403.307 | 6.59 | 0.86 |
| Na | 589.592 | 6.42 | 0.18 |

ND= Not Detectable

Table S3. ICP analysis of dialyzed SSF C1

| Element | Wavelength (nm) | Concentration (mg/Kg) | %RSD |
| --- | --- | --- | --- |
| Al | 394.401 | 0.04 | 2.09 |
| P | 214.915 | ND |  |
| Se | 206.275 | ND |  |
| Zn | 213.857 | 0.49 | 0.30 |
| Fe | 373.486 | 0.09 | 0.08 |
| Ca | 422.673 | 9.45 | 0.14 |
| Ba | 553.548 | 0.16 | 0.27 |
| Cu | 324.754 | 0.09 | 14.63 |
| Ni | 341.476 361.939 | ND ND |  |
| K | 769.897 | 2.59 | 0.33 |
| Pb | 405.781 | 0.01 | 10.31 |
| Cr | 425.433 | 0.004 | 2.10 |
| Mg | 383.829 | 0.46 | 0.34 |
| Mn | 403.449 | 0.005 | 1.80 |
| Na | 589.592 | 2.05 | 1.19 |

ND= Not Detectable

Table S4. ICP analysis of dialyzed SSF C2

| Element | Wavelength (nm) | Concentration (mg/Kg) | %RSD |
| --- | --- | --- | --- |
| Al | 394.401 | 0.32 | 28.58 |
| P | 213.618 | 14.69 | 0.95 |
| Se | 206.275 | 19.05 | 4.84 |
| Zn | 213.857 | 0.57 | 1.37 |
| Fe | 371.993 | 0.09 | 3.91 |
| Ca | 422.673 | 3.02 | 1.54 |
| Ba | 705.994 | 0.15 | 0.90 |
| Cu | 327.395 | 0.95 | 2.49 |
| Ni | 361.939 | 0.05 | 0.71 |
| K | 769.897 | 8.36 | 1.05 |
| Pb | 405.781 | 0.11 | 11.18 |
| Cr | 425.433 | 0.10 | 1.12 |
| Mg | 285.213 | 0.24 | 1.37 |
| Mn | 403.307 | 0.008 | 1.03 |
| Na | 589.592 | ND |  |

ND= Not Detectable