Supplementary material for

Simultaneous removal of Eriochrome Black T and chromate anions from aqueous solution using functionalized magnetic polymers

Huda M. Alghamdi, Rihab M. Mohammad, Khalid Z. Elwakeel

University of Jeddah, College of Science, Department of Chemistry, Jeddah, Saudi Arabia.

Table S1. BET surface area, pore volume and pore diameter of R-DETA and R-Dithizone adsorbents

| Adsorbent | BET surface area (m2 g-1)* | Pore volume (cm3 g-1) ** | Pore diameter (Å) ** |
| --- | --- | --- | --- |
| R-DETA | 11.0 | 0.207 | 7.5 |
| R-Dithizone | 9.5 | 0.192 | 6.3 |

*BET specific surface area measured by multipoint method.

**Pore volume and pore radius calculated with BJH method on N2 desorption

Table S2. Elemental analysis of MCGMA and R-DETA and R-Dithizone adsorbents

| Adsorbent | C (%) | H (%) | N (%) | N (mmol g-1) | O (%) | S (%) | S (mmol g-1) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| MCGMA | 36.10 | 7.00 | 4.40 | 3.14 | 25.6 | - | - |
| R-DETA | 31.16 | 5.94 | 14.01 | 10.0 | 24.72 | - | - |
| R-Dithizone | 39.26 | 4.99 | 10.14 | 7.24 | 17.50 | 3.77 | 1.17 |

Table S3. The adsorption capacities of different adsorbents regarding Cr(VI) and EBT

| Adsorbent | Pollutant | pH | Qmax (mg g-1) | Equilibrium time (min) | Temp. (oC) | Reference |
| --- | --- | --- | --- | --- | --- | --- |
| Chitosan-SiO2-TiO2 | Cr(VI) | 3 | 182.43 | 120 | 25 ± 1 | [1] |
| Ionic liquid filled chitosan capsules | Cr(VI) | 2 | 110.94 ± 5.07 |  | 20 ± 1 | [2] |
| Chitosan/ploy (vinyl alcohol) porous microspheres were successfully prepared throughgelation and freeze-drying process | Cr(VI) | 3 | 334.7 | 60 | 25 ± 1 | [3] |
| Zirconium-based MOF and chitosan composites | Cr(VI) | 5 | 320.0 | 30 | 25 ± 1 | [4] |
| Zr4+ cross-linked chitosan-thiourea composite | Cr(VI) | 2 | 246.72 289.47 323.86 | 90 | 25 ± 1 35 ± 1 40 ± 1 | [5] |
| Poly[(glycidyl methacrylate)-co-(ethylene glycol dimethacrylate)] | Cr(VI) | 2 | 214 | 60 | 70 ± 1 | [6] |
| Ethylenediaminetetraacetic -crosslinking-chitosan/polypyrrole | Cr(VI) | 6 | 401.25 |  | 25 ± 1 | [7] |
| Activated carbon derived from Eichhornia crassipes | Cr(VI) | 5 | 26.66 | 90 | 25 ± 1 | [8] |
| Coffee Polyphenol-Formaldehyde/Acetaldehyde Resin | Cr(VI) | 2 |  | 150 | 25 ± 1 | [9] |
| SiO2/polyaniline composite | Cr(VI) | 5-6 | 285.5 | 60 | - | [10] |
| R-DETA | Cr(VI) | 3.3 | 192.90 | 180 | 25 ± 1 | This study |
| R-Dithizone | Cr(VI) | 3.3 | 227.74 | 180 | 25 ± 1 | This study |
| SiO2/polyaniline composite | EBT | 5-6 | 90.23 | 60 | - | [10] |
| # Acid and alkaline activated volcanic ash-based geopolymers. Acid activation (GPAc); alkaline activation (GPAlk) | EBT | 3-6 | GPAc = 10.34 GPAlk = 8.15 | 30 | 25 ± 1 | [11] |
| Sodium zinc phosphate/polyaniline nanocomposite | EBT | 2 | 234.4 | 150 | - | [12] |
| MgCO3/MnCO3 (Abbreviated as MC) and MgMn2O4/Mn2O3 (Abbreviated as MO) | EBT | 3 | MC= 416.67 MO= 386.10 | - | 25 ± 1 | [13] |
| R-DETA | EBT | 3.3 | 323.4281 | 180 | 25 ± 1 | This study |
| R-Dithizone | EBT | 3.3 | 199.3166 | 180 | 25 ± 1 | This study |

Scheme S1: Eriochrome Black T chemical structure

Figure S1: TEM images of magnetite NPs

| R-DETA | R-Dithizone |
| --- | --- |

Figure S2: SEM photos of R- DETA (left column) and R-Dithizone adsorbents (right column).

| R-DETA | R-Dithizone |
| --- | --- |

Figure S3: TEM photos of R- DETA (left column) and R-Dithizone adsorbents (right column).

Figure S4: Nitrogen  adsorption/desorption curves of R-DETA and R-Dithizone adsorbents.

Figure S5: Vibrating sample magnetometry (VSM) curves for Fe3O4 NPs, MCGMA, R-DETA and R-Dithizone adsorbents

Figure S6: XRD patterns for MCGMA, R-DETA and R-Dithizone

Figure S7: Differential light scattering (DLS) for Fe3O4 NPs, MCGMA, R-DETA and R-Dithizone adsorbents

Figure S8: Thermogravimetric analysis (TGA) of R-DETA and R-Dithizone sorbents

Figure S9: FTIR spectra of R-DETA and R-Dithizone adsorbents.

Figure S10: Zeta potential plots for R-DETA and R-Dithizone adsorbents

Figure S11: Chormium(VI) speciation at different pH values  [9]

Figure S12: Linear sorption isotherms of EBT and Cr(VI) sorption from their binary solution on R-DETA (Sorbent mass 0.05 g; V: 0.025 L; t: 180 min; temperature: 25 ± 1°C; agitation speed: 200 rpm; pH0: 3.3).

Figure S13: Linear sorption isotherms of EBT and Cr(VI) sorption from their binary solution on R-dithizone (Sorbent mass 0.05 g; V: 0.025 L; t: 180 min; temperature: 25 ± 1°C; agitation speed: 200 rpm; pH0: 3.3).

References

[1] R. El Kaim Billah, A. Shekhawat, S. Mansouri, H. Majdoubi, M. Agunaou, A. Soufiane, R. Jugade, Adsorptive removal of Cr(VI) by Chitosan-SiO2-TiO2 nanocomposite, Environ. Nanotechnol. Monit. Manag. 18 (2022) 100695. https://doi.org/10.1016/j.enmm.2022.100695.

[2] X. Lin, X. He, L. Lei, Y. Zhao, L. Cui, G. Wu, Development of ionic liquid filled chitosan capsules to remove Cr(VI) from acidic solution: Adsorption properties and mechanism, J. Environ. Chem. Eng. 10(4) (2022) 108081. https://doi.org/10.1016/j.jece.2022.108081.

[3] W. Song, T. Tong, J. Xu, N. Wu, L. Ren, M. Li, J. Tong, Preparation and application of green chitosan/ploy (vinyl alcohol) porous microspheres for the removal of hexavalent chromium, Materials Science and Engineering: B 284 (2022) 115922. https://doi.org/10.1016/j.mseb.2022.115922.

[4] F.M. Valadi, S. Shahsavari, E. Akbarzadeh, M.R. Gholami, Preparation of new MOF-808/chitosan composite for Cr(VI) adsorption from aqueous solution: Experimental and DFT study, Carbohydr. Polym. 288 (2022) 119383. https://doi.org/10.1016/j.carbpol.2022.119383.

[5] C. Xu, Y. Xu, D. Zhong, H. Chang, J. Mou, H. Wang, H. Shen, Zr4+ cross-linked chitosan-thiourea composite for efficient detoxification of Cr(VI) ions in aqueous solution, Carbohydr. Polym. 296 (2022) 119872. https://doi.org/10.1016/j.carbpol.2022.119872.

[6] B.M. Marković, I.S. Stefanović, R.V. Hercigonja, M.V. Pergal, J.P. Marković, A.E. Onjia, A.B. Nastasović, Novel hexamethylene diamine-functionalized macroporous copolymer for chromium removal from aqueous solutions, Polym. Int. 66(5) (2017) 679-689. https://doi.org/10.1002/pi.5306.

[7] Y. Shi, J. Feng, Z. Zhang, N. Cao, J. Li, H. Li, L. Li, Q. Hua, Q. Ma, K. Zhang, Simultaneous removal of Cr(VI) anions and metal cations by EDTA-crosslinking-chitosan/polypyrrole composites, Sep. Purif. Technol. 327 (2023) 124926. https://doi.org/10.1016/j.seppur.2023.124926.

[8] J. Fito, S. Tibebu, T.T.I. Nkambule, Optimization of Cr (VI) removal from aqueous solution with activated carbon derived from Eichhornia crassipes under response surface methodology, BMC Chemistry 17(1) (2023) 4. 10.1186/s13065-023-00913-6.

[9] K. Mulani, S. Daniels, K. Rajdeo, S. Tambe, N. Chavan, Adsorption of chromium (VI) from aqueous solutions by coffee polyphenol-formaldehyde/acetaldehyde resins, Journal of Polymers 2013 (2013).

[10] H. Hajjaoui, A. Soufi, M. Khnifira, M. Abdennouri, F.Z. Mahjoubi, N. Barka, Mono and binary mixture removal of eriochrome black T and Cr(VI) from water by SiO2/polyaniline composite, Mater. Chem. Phys. 296 (2023) 127220. https://doi.org/10.1016/j.matchemphys.2022.127220.

[11] S. Tome, D.T. Hermann, V.O. Shikuku, S. Otieno, Synthesis, characterization and application of acid and alkaline activated volcanic ash-based geopolymers for adsorptive remotion of cationic and anionic dyes from water, Ceram. Int. 47(15) (2021) 20965-20973. https://doi.org/10.1016/j.ceramint.2021.04.097.

[12] H. Hajjaoui, A. Soufi, H. Khiar, M. Abdennouri, M. Achak, N. Barka, Preparation of sodium zinc phosphate/polyaniline nanocomposite for Cr(VI) and eriochrome black T adsorption from water, Mater. Today Commun. 36 (2023) 106755. https://doi.org/10.1016/j.mtcomm.2023.106755.

[13] N.S. Al-Kadhi, F.A. Saad, R.K. Shah, E.S. Al-Farraj, G.S. El-Sayyad, E.A. Abdelrahman, A Facile Sol-gel Synthesis and Characterization of MgCO3/MnCO3 and MgMn2O4/Mn2O3 Novel Nanostructures With Remarkably High Adsorption Activity Toward Eriochrome Black T Dye, J. Inorg. Organomet .Polym. Mater. 33(7) (2023) 2046-2057. 10.1007/s10904-023-02660-6.

Corresponding author:

University of Jeddah, College of Science, Department of Chemistry, Jeddah, Saudi Arabia (K.Z. Elwakeel).

E-mail address: kelwkeel@uj.edu.sa