Enhancing thermo-physical properties of hybrid nanoparticle-infused RT-54HC organic PCMs using graphene nanoplatelets and multiwall carbon nanotubes
Anas Islam1*, A.K Pandey1*, Kamal Sharma2, Yasir Ali Bhutto1, R. Saidur1,3, D. Buddhi4
1 Research Centre for Nanomaterials and Energy Technology (RCNMET), School of Engineering and Technology, Sunway University, No. 5, Jalan Universiti, Bandar Sunway, Petaling Jaya, 47500 Selangor Darul Ehsan, Malaysia
2 Department of Mechanical Engineering, Institute of Engineering and Technology, GLA University, Mathura 281406, India
3 School of Engineering, Lancaster University, Lancaster, LA1 4YW UK
4 CoE for Energy and Eco-sustainaibility Research, Uttaranchal University Dehradun Uttarakhand India 248007
* anas.i2@imail.sunway.edu.my

1. DSC data








2. FTIR







3. UV-Vis







4. TGA







image3.emf
RT54-0.2 MWCNT.txt


RT54-0.2 MWCNT.txt
# Name: RT54-0.2 MWCNT

# Date: Tue May 21 17:29:18 2024

# Weight: 11.8 mg

Time(s)	Temperature(°C)	Heat flow(mW)	Gas 1(sccm/min)	DSC_RAW(µV)	POWER(%)	TEMP_CJR_FURNACE(K)	TEMP_CJR_SAMPLE(K)	TEMP_FURNACE(K)	TEMP_NOM_FURNACE(K)	TEMP_NOM_SAMPLE(K)	VOLTAGE_REFERENCE(V)	VOLTAGE_SAMPLE(V)

0	29.83	0.163419	19.9987	0.000222426	0.0712991	293.15	293.15	0	303.265	303.265	0.068538	0.0684937

1	29.87	0.516549	19.9904	0.000703054	0.128672	293.15	293.15	0	303.434	303.434	0.0685462	0.0685025

2	29.96	0.501386	19.9977	0.000682396	0.174963	293.15	293.15	0	303.611	303.611	0.0685668	0.068524

3	30.09	-0.152443	20.0008	-0.00020747	0.203393	293.15	293.15	0	303.775	303.775	0.0685959	0.0685564

4	30.25	-1.33332	20.0008	-0.00181452	0.224118	293.15	293.15	0	303.935	303.935	0.0686314	0.0685942

5	30.43	-2.75056	20.006	-0.00374303	0.240076	293.15	293.15	0	304.106	304.106	0.06867	0.0686353

6	30.61	-4.23352	20.0008	-0.00576076	0.253978	293.15	293.15	0	304.272	304.272	0.0687108	0.0686785

7	30.81	-5.66287	20.0008	-0.00770528	0.258109	293.15	293.15	0	304.426	304.426	0.068756	0.0687256

8	31	-6.85962	20.0008	-0.00933311	0.262216	293.15	293.15	0	304.599	304.599	0.0688006	0.0687716

9	31.2	-7.88386	20.0008	-0.010726	0.268961	293.15	293.15	0	304.773	304.773	0.0688456	0.0688175

10	31.39	-8.70247	20.0008	-0.0118391	0.269098	293.15	293.15	0	304.947	304.947	0.0688913	0.0688632

11	31.58	-9.20143	20.0008	-0.0125171	0.269016	293.15	293.15	0	305.094	305.094	0.0689363	0.0689087

12	31.77	-9.50436	20.0008	-0.0129285	0.269291	293.15	293.15	0	305.267	305.267	0.068981	0.0689534

13	31.96	-9.70982	20.0008	-0.0132072	0.267913	293.15	293.15	0	305.431	305.431	0.0690262	0.0689985

14	32.15	-9.907	20.0008	-0.0134746	0.27174	293.15	293.15	0	305.602	305.602	0.0690699	0.0690429

15	32.33	-10.0166	20.0008	-0.0136229	0.272446	293.15	293.15	0	305.768	305.768	0.0691127	0.0690855

16	32.51	-10.075	20.0008	-0.0137016	0.272331	293.15	293.15	0	305.934	305.934	0.069156	0.0691282

17	32.69	-10.0359	20.0008	-0.0136477	0.274514	293.15	293.15	0	306.095	306.095	0.0691976	0.0691707

18	32.86	-9.90137	20.0008	-0.013464	0.276963	293.15	293.15	0	306.271	306.271	0.0692387	0.0692117

19	33.04	-9.75657	20.0008	-0.0132664	0.279164	293.15	293.15	0	306.435	306.435	0.0692805	0.0692536

20	33.21	-9.62392	20.0008	-0.0130853	0.279597	293.15	293.15	0	306.604	306.604	0.0693217	0.0692949

21	33.39	-9.54266	20.0008	-0.0129742	0.282039	293.15	293.15	0	306.765	306.765	0.0693628	0.0693365

22	33.56	-9.50088	20.0008	-0.0129167	0.286463	293.15	293.15	0	306.932	306.932	0.0694032	0.0693763

23	33.72	-9.4294	20.0008	-0.0128189	0.290444	293.15	293.15	0	307.102	307.102	0.0694426	0.0694161

24	33.9	-9.39558	20.0008	-0.0127722	0.292784	293.15	293.15	0	307.276	307.276	0.0694833	0.0694575

25	34.07	-9.39841	20.0008	-0.0127754	0.295924	293.15	293.15	0	307.441	307.441	0.0695233	0.0694979

26	34.24	-9.38798	20.0008	-0.0127605	0.297812	293.15	293.15	0	307.609	307.609	0.0695637	0.0695381

27	34.41	-9.36678	20.0008	-0.0127311	0.300803	293.15	293.15	0	307.769	307.769	0.0696033	0.069578

28	34.58	-9.36049	20.0008	-0.0127219	0.302853	293.15	293.15	0	307.935	307.935	0.0696431	0.0696179

29	34.74	-9.33132	20.0008	-0.0126816	0.304194	293.15	293.15	0	308.099	308.099	0.0696827	0.0696572

30	34.91	-9.32023	20.0008	-0.0126659	0.31122	293.15	293.15	0	308.264	308.264	0.0697216	0.0696966

31	35.08	-9.30254	20.0008	-0.0126412	0.312917	293.15	293.15	0	308.437	308.437	0.0697625	0.0697368

32	35.25	-9.30899	19.9904	-0.0126493	0.312092	293.15	293.15	0	308.601	308.601	0.0698024	0.0697769

33	35.42	-9.20066	19.9998	-0.0125014	0.316949	293.15	293.15	0	308.767	308.767	0.0698414	0.0698165

34	35.58	-9.16524	20.0008	-0.0124527	0.321319	293.15	293.15	0	308.939	308.939	0.0698804	0.0698562

35	35.75	-9.22906	20.0008	-0.0125387	0.323789	293.15	293.15	0	309.104	309.104	0.0699208	0.069895

36	35.92	-9.25822	20.0008	-0.0125777	0.32877	293.15	293.15	0	309.277	309.277	0.0699595	0.0699357

37	36.09	-9.25524	20.0008	-0.012573	0.330416	293.15	293.15	0	309.425	309.425	0.0699987	0.069975

38	36.25	-9.3039	19.9956	-0.0126385	0.334623	293.15	293.15	0	309.594	309.594	0.0700385	0.0700148

39	36.42	-9.34237	20.0008	-0.0126901	0.337242	293.15	293.15	0	309.771	309.771	0.070078	0.0700545

40	36.59	-9.33385	20.0008	-0.0126779	0.337977	293.15	293.15	0	309.941	309.941	0.0701185	0.0700951

41	36.76	-9.35293	20.0008	-0.0127031	0.341089	293.15	293.15	0	310.108	310.108	0.0701577	0.070133

42	36.92	-9.37443	20.0008	-0.0127317	0.345789	293.15	293.15	0	310.274	310.274	0.0701962	0.0701728

43	37.09	-9.3567	19.9935	-0.012707	0.351528	293.15	293.15	0	310.433	310.433	0.070235	0.0702123

44	37.25	-9.28664	19.9977	-0.0126112	0.354602	293.15	293.15	0	310.602	310.602	0.0702742	0.0702511

45	37.42	-9.22387	20.0008	-0.0125253	0.358687	293.15	293.15	0	310.776	310.776	0.0703141	0.0702903

46	37.59	-9.24204	20.0008	-0.0125493	0.360697	293.15	293.15	0	310.935	310.935	0.0703533	0.0703307

47	37.76	-9.33115	20.0008	-0.0126697	0.362081	293.15	293.15	0	311.096	311.096	0.0703932	0.0703703

48	37.93	-9.38408	20.0008	-0.0127409	0.365971	293.15	293.15	0	311.271	311.271	0.0704329	0.0704109

49	38.09	-9.41205	20.0008	-0.0127782	0.371118	293.15	293.15	0	311.444	311.444	0.0704707	0.0704488

50	38.26	-9.4703	20.0008	-0.0128566	0.370546	293.15	293.15	0	311.608	311.608	0.0705109	0.0704886

51	38.43	-9.49975	20.0008	-0.012896	0.377307	293.15	293.15	0	311.763	311.763	0.0705506	0.0705291

52	38.6	-9.53704	20.0112	-0.0129459	0.378159	293.15	293.15	0	311.946	311.946	0.0705903	0.0705686

53	38.77	-9.58604	20.0008	-0.0130118	0.382755	293.15	293.15	0	312.11	312.11	0.0706284	0.0706079

54	38.93	-9.57268	20.0008	-0.012993	0.385534	293.15	293.15	0	312.283	312.283	0.0706686	0.0706474

55	39.1	-9.52562	20.005	-0.0129285	0.389716	293.15	293.15	0	312.44	312.44	0.070707	0.0706864

56	39.27	-9.49008	20.0112	-0.0128795	0.389989	293.15	293.15	0	312.597	312.597	0.0707473	0.0707266

57	39.43	-9.53202	20.0029	-0.0129358	0.396236	293.15	293.15	0	312.766	312.766	0.0707861	0.0707655

58	39.6	-9.59978	19.9956	-0.0130271	0.399944	293.15	293.15	0	312.935	312.935	0.0708254	0.0708047

59	39.77	-9.64983	20.0008	-0.0130944	0.403009	293.15	293.15	0	313.108	313.108	0.070864	0.0708444

60	39.94	-9.66805	20.0008	-0.0131184	0.405946	293.15	293.15	0	313.267	313.267	0.0709039	0.0708845

61	40.1	-9.69984	19.9987	-0.0131609	0.409043	293.15	293.15	0	313.428	313.428	0.070944	0.0709239

62	40.27	-9.69839	19.9904	-0.0131582	0.412436	293.15	293.15	0	313.601	313.601	0.0709834	0.0709635

63	40.44	-9.65203	19.9977	-0.0130947	0.414416	293.15	293.15	0	313.769	313.769	0.0710234	0.0710028

64	40.61	-9.63471	20.0008	-0.0130705	0.420267	293.15	293.15	0	313.938	313.938	0.0710623	0.0710424

65	40.77	-9.64976	20.0008	-0.0130903	0.425296	293.15	293.15	0	314.111	314.111	0.071101	0.0710815

66	40.94	-9.66112	20.006	-0.013105	0.427238	293.15	293.15	0	314.268	314.268	0.0711403	0.0711203

67	41.1	-9.6993	19.9914	-0.0131561	0.428949	293.15	293.15	0	314.425	314.425	0.0711793	0.0711598

68	41.27	-9.83266	20.0008	-0.0133363	0.432996	293.15	293.15	0	314.608	314.608	0.0712181	0.0711994

69	41.44	-9.84586	20.0008	-0.0133536	0.438409	293.15	293.15	0	314.762	314.762	0.0712574	0.0712392

70	41.61	-9.83303	20.0008	-0.0133355	0.438779	293.15	293.15	0	314.935	314.935	0.0712975	0.0712781

71	41.77	-9.84566	19.9904	-0.0133519	0.441012	293.15	293.15	0	315.1	315.1	0.0713367	0.0713177

72	41.94	-9.8608	19.9956	-0.0133718	0.445598	293.15	293.15	0	315.283	315.283	0.0713758	0.0713572

73	42.11	-9.85139	20.0008	-0.0133583	0.448749	293.15	293.15	0	315.43	315.43	0.0714152	0.0713971

74	42.28	-9.80571	20.0008	-0.0132957	0.453385	293.15	293.15	0	315.603	315.603	0.071454	0.0714362

75	42.44	-9.78293	20.0008	-0.0132642	0.457028	293.15	293.15	0	315.767	315.767	0.0714932	0.0714751

76	42.61	-9.838	20.0008	-0.0133382	0.460519	293.15	293.15	0	315.938	315.938	0.0715316	0.0715144

77	42.77	-9.86397	20.0008	-0.0133727	0.467525	293.15	293.15	0	316.104	316.104	0.071571	0.0715536

78	42.95	-9.89573	20.0008	-0.013415	0.469185	293.15	293.15	0	316.275	316.275	0.0716113	0.0715941

79	43.11	-9.90468	20.0008	-0.0134265	0.471711	293.15	293.15	0	316.434	316.434	0.0716501	0.0716335

80	43.28	-9.9075	20.0008	-0.0134296	0.474747	293.15	293.15	0	316.607	316.607	0.0716891	0.0716722

81	43.44	-9.93044	20.0008	-0.0134601	0.479246	293.15	293.15	0	316.771	316.771	0.0717284	0.0717117

82	43.61	-9.93391	20.0008	-0.0134641	0.481201	293.15	293.15	0	316.932	316.932	0.0717687	0.0717519

83	43.78	-9.92909	20.0008	-0.0134568	0.483588	293.15	293.15	0	317.092	317.092	0.0718077	0.0717915

84	43.95	-9.91007	20.0008	-0.0134304	0.487577	293.15	293.15	0	317.269	317.269	0.0718476	0.0718312

85	44.12	-9.90576	20.0008	-0.0134238	0.494245	293.15	293.15	0	317.438	317.438	0.0718864	0.0718711

86	44.28	-9.92759	20.0029	-0.0134527	0.499281	293.15	293.15	0	317.611	317.611	0.0719246	0.0719097

87	44.45	-9.97651	20.0112	-0.0135183	0.50046	293.15	293.15	0	317.76	317.76	0.0719649	0.0719493

88	44.62	-10.0578	20.0039	-0.0136278	0.503227	293.15	293.15	0	317.926	317.926	0.072004	0.0719892

89	44.79	-10.1185	19.9914	-0.0137094	0.504907	293.15	293.15	0	318.106	318.106	0.0720436	0.0720286

90	44.95	-10.1122	20.0008	-0.0137002	0.510264	293.15	293.15	0	318.272	318.272	0.0720825	0.0720677

91	45.12	-10.1032	20.0008	-0.0136872	0.512556	293.15	293.15	0	318.427	318.427	0.072122	0.0721069

92	45.29	-10.1333	20.0008	-0.0137273	0.514919	293.15	293.15	0	318.599	318.599	0.0721603	0.0721465

93	45.46	-10.1367	20.0008	-0.0137312	0.521401	293.15	293.15	0	318.763	318.763	0.0722002	0.0721857

94	45.62	-10.1686	20.0008	-0.0137738	0.52265	293.15	293.15	0	318.937	318.937	0.0722391	0.0722251

95	45.79	-10.1998	20.0102	-0.0138153	0.525277	293.15	293.15	0	319.093	319.093	0.0722784	0.0722645

96	45.96	-10.2407	20.0019	-0.01387	0.53012	293.15	293.15	0	319.274	319.274	0.0723177	0.0723039

97	46.13	-10.298	20.0008	-0.0139469	0.532319	293.15	293.15	0	319.441	319.441	0.0723579	0.0723433

98	46.29	-10.3462	20.0008	-0.0140114	0.534778	293.15	293.15	0	319.606	319.606	0.0723962	0.0723827

99	46.46	-10.3797	19.9925	-0.0140561	0.540927	293.15	293.15	0	319.76	319.76	0.0724357	0.0724226

100	46.63	-10.3799	19.9987	-0.0140556	0.544522	293.15	293.15	0	319.939	319.939	0.0724743	0.0724614

101	46.79	-10.3109	20.0008	-0.0139615	0.547592	293.15	293.15	0	320.091	320.091	0.072514	0.0725001

102	46.96	-10.3048	20.0008	-0.0139526	0.553224	293.15	293.15	0	320.258	320.258	0.0725525	0.0725394

103	47.13	-10.3271	20.0008	-0.013982	0.556876	293.15	293.15	0	320.437	320.437	0.0725921	0.072579

104	47.3	-10.3601	20.0008	-0.0140259	0.560257	293.15	293.15	0	320.605	320.605	0.0726313	0.0726187

105	47.46	-10.3564	19.9956	-0.0140203	0.565502	293.15	293.15	0	320.774	320.774	0.0726694	0.0726569

106	47.63	-10.347	19.9998	-0.0140068	0.565506	293.15	293.15	0	320.93	320.93	0.0727099	0.072698

107	47.8	-10.3759	19.9904	-0.0140452	0.571869	293.15	293.15	0	321.095	321.095	0.0727492	0.0727369

108	47.97	-10.3909	19.9966	-0.0140648	0.573364	293.15	293.15	0	321.261	321.261	0.0727886	0.0727764

109	48.13	-10.3363	20.0008	-0.0139902	0.575334	293.15	293.15	0	321.442	321.442	0.0728278	0.0728154

110	48.3	-10.2926	20.0008	-0.0139304	0.577832	293.15	293.15	0	321.598	321.598	0.0728671	0.0728546

111	48.46	-10.3616	20.0008	-0.0140231	0.584392	293.15	293.15	0	321.762	321.762	0.0729058	0.0728936

112	48.63	-10.3988	20.0112	-0.0140727	0.586561	293.15	293.15	0	321.935	321.935	0.0729449	0.0729327

113	48.8	-10.3337	20.0008	-0.0139838	0.58923	293.15	293.15	0	322.1	322.1	0.0729842	0.0729719

114	48.96	-10.3083	20.0008	-0.0139488	0.593153	293.15	293.15	0	322.273	322.273	0.0730231	0.0730113

115	49.13	-10.3151	20.0008	-0.0139572	0.59811	293.15	293.15	0	322.438	322.438	0.0730625	0.0730508

116	49.3	-10.3411	19.9946	-0.0139918	0.602167	293.15	293.15	0	322.601	322.601	0.0731013	0.0730899

117	49.46	-10.3672	20.0008	-0.0140264	0.607254	293.15	293.15	0	322.759	322.759	0.0731394	0.0731285

118	49.64	-10.4229	20.0008	-0.014101	0.608621	293.15	293.15	0	322.938	322.938	0.0731797	0.073169

119	49.8	-10.4644	20.0008	-0.0141564	0.614866	293.15	293.15	0	323.106	323.106	0.0732191	0.0732083

120	49.97	-10.5195	20.0008	-0.0142303	0.616825	293.15	293.15	0	323.272	323.272	0.0732586	0.0732478

121	50.14	-10.5549	20.0008	-0.0142774	0.619713	293.15	293.15	0	323.43	323.43	0.0732973	0.0732874

122	50.3	-10.5196	20.0008	-0.0142289	0.623675	293.15	293.15	0	323.6	323.6	0.0733363	0.0733259

123	50.47	-10.4677	20.0008	-0.014158	0.629159	293.15	293.15	0	323.774	323.774	0.0733753	0.0733654

124	50.63	-10.4791	20.0008	-0.0141727	0.633961	293.15	293.15	0	323.932	323.932	0.0734134	0.0734035

125	50.8	-10.5045	20.0008	-0.0142063	0.638285	293.15	293.15	0	324.103	324.103	0.0734528	0.0734431

126	50.97	-10.5073	20.0008	-0.0142094	0.640904	293.15	293.15	0	324.269	324.269	0.0734916	0.0734828

127	51.14	-10.5526	20.0008	-0.01427	0.64269	293.15	293.15	0	324.424	324.424	0.0735315	0.073523

128	51.31	-10.5607	19.9904	-0.0142801	0.647033	293.15	293.15	0	324.597	324.597	0.0735718	0.0735624

129	51.48	-10.5827	20.0008	-0.0143092	0.651652	293.15	293.15	0	324.77	324.77	0.07361	0.0736015

130	51.64	-10.5992	20.0008	-0.0143308	0.652783	293.15	293.15	0	324.944	324.944	0.0736494	0.0736408

131	51.81	-10.6536	20.0008	-0.0144036	0.655779	293.15	293.15	0	325.091	325.091	0.0736883	0.0736801

132	51.98	-10.6701	20.0008	-0.0144252	0.660748	293.15	293.15	0	325.272	325.272	0.0737278	0.0737198

133	52.15	-10.6834	20.0008	-0.0144424	0.665903	293.15	293.15	0	325.437	325.437	0.0737666	0.0737588

134	52.31	-10.687	20.0008	-0.0144465	0.669182	293.15	293.15	0	325.603	325.603	0.0738065	0.073798

135	52.48	-10.6876	20.0008	-0.0144466	0.672802	293.15	293.15	0	325.763	325.763	0.0738443	0.0738367

136	52.64	-10.6794	20.0008	-0.0144348	0.675489	293.15	293.15	0	325.931	325.931	0.0738837	0.0738758

137	52.81	-10.7114	20.0008	-0.0144773	0.681211	293.15	293.15	0	326.104	326.104	0.0739228	0.0739149

138	52.98	-10.7708	20.0008	-0.0145568	0.684992	293.15	293.15	0	326.265	326.265	0.0739617	0.0739543

139	53.15	-10.8157	19.9987	-0.0146168	0.690402	293.15	293.15	0	326.435	326.435	0.0740005	0.0739936

140	53.31	-10.7993	19.9904	-0.0145938	0.692521	293.15	293.15	0	326.602	326.602	0.0740401	0.0740328

141	53.48	-10.7519	19.9977	-0.0145291	0.696384	293.15	293.15	0	326.772	326.772	0.0740794	0.0740729

142	53.65	-10.7488	20.0008	-0.0145242	0.703238	293.15	293.15	0	326.937	326.937	0.0741183	0.0741121

143	53.82	-10.8463	20.0008	-0.0146551	0.705435	293.15	293.15	0	327.092	327.092	0.0741573	0.0741511

144	53.99	-10.9403	19.9998	-0.0147815	0.705765	293.15	293.15	0	327.267	327.267	0.0741971	0.0741917

145	54.16	-11.0296	19.9914	-0.0149014	0.709557	293.15	293.15	0	327.439	327.439	0.0742362	0.0742306

146	54.32	-11.0762	20.0008	-0.0149636	0.715649	293.15	293.15	0	327.596	327.596	0.0742745	0.0742687

147	54.49	-11.0838	20.0008	-0.014973	0.717858	293.15	293.15	0	327.76	327.76	0.0743142	0.0743083

148	54.65	-11.081	20.0008	-0.0149685	0.721159	293.15	293.15	0	327.933	327.933	0.0743529	0.0743476

149	54.82	-11.0913	20.0008	-0.0149816	0.729348	293.15	293.15	0	328.097	328.097	0.0743914	0.0743859

150	54.99	-11.1422	19.9966	-0.0150497	0.730686	293.15	293.15	0	328.271	328.271	0.0744309	0.0744264

151	55.16	-11.2122	19.9998	-0.0151434	0.733024	293.15	293.15	0	328.427	328.427	0.0744702	0.074466

152	55.32	-11.286	20.006	-0.0152423	0.73792	293.15	293.15	0	328.601	328.601	0.074509	0.0745046

153	55.49	-11.347	20.0008	-0.0153239	0.742391	293.15	293.15	0	328.772	328.772	0.0745478	0.0745435

154	55.66	-11.4278	20.0008	-0.0154323	0.748453	293.15	293.15	0	328.937	328.937	0.0745862	0.0745825

155	55.82	-11.5038	19.9966	-0.015534	0.751812	293.15	293.15	0	329.11	329.11	0.0746259	0.0746222

156	55.99	-11.5713	19.9904	-0.0156245	0.756228	293.15	293.15	0	329.272	329.272	0.0746644	0.0746612

157	56.16	-11.6511	19.9987	-0.0157315	0.759532	293.15	293.15	0	329.431	329.431	0.0747026	0.0747003

158	56.33	-11.7285	20.0008	-0.0158352	0.763821	293.15	293.15	0	329.604	329.604	0.0747428	0.0747407

159	56.5	-11.8282	20.0008	-0.0159689	0.768042	293.15	293.15	0	329.773	329.773	0.0747817	0.0747798

160	56.66	-11.9658	20.0008	-0.0161538	0.771515	293.15	293.15	0	329.933	329.933	0.07482	0.074819

161	56.83	-12.1661	19.9956	-0.0164234	0.777678	293.15	293.15	0	330.099	330.099	0.0748592	0.0748574

162	56.99	-12.3826	20.0008	-0.0167148	0.784645	293.15	293.15	0	330.266	330.266	0.0748974	0.0748965

163	57.16	-12.5469	20.0008	-0.0169358	0.789014	293.15	293.15	0	330.435	330.435	0.0749361	0.0749357

164	57.33	-12.7191	20.0008	-0.0171673	0.794713	293.15	293.15	0	330.609	330.609	0.0749749	0.0749746

165	57.5	-12.9517	20.0008	-0.0174804	0.800597	293.15	293.15	0	330.774	330.774	0.0750136	0.0750147

166	57.67	-13.2528	20.0019	-0.0178858	0.804766	293.15	293.15	0	330.922	330.922	0.0750526	0.0750544

167	57.84	-13.6445	20.0102	-0.0184136	0.811396	293.15	293.15	0	331.103	331.103	0.0750908	0.0750937

168	58	-14.1267	20.0008	-0.0190633	0.817399	293.15	293.15	0	331.269	331.269	0.075128	0.0751319

169	58.17	-14.7326	20.0008	-0.0198799	0.823473	293.15	293.15	0	331.424	331.424	0.0751659	0.0751714

170	58.33	-15.4834	20.0008	-0.020892	0.835165	293.15	293.15	0	331.597	331.597	0.0752028	0.0752092

171	58.49	-16.4369	20.0008	-0.0221776	0.845918	293.15	293.15	0	331.77	331.77	0.0752389	0.0752475

172	58.66	-17.6599	20.0008	-0.0238265	0.857528	293.15	293.15	0	331.943	331.943	0.0752749	0.0752861

173	58.83	-19.2068	20.0008	-0.0259122	0.868193	293.15	293.15	0	332.108	332.108	0.0753111	0.0753254

174	58.99	-21.0811	20.0008	-0.0284394	0.885821	293.15	293.15	0	332.274	332.274	0.0753455	0.075363

175	59.15	-23.3778	20.0008	-0.0315363	0.905568	293.15	293.15	0	332.435	332.435	0.075379	0.0754009

176	59.31	-26.0687	20.0102	-0.0351646	0.92448	293.15	293.15	0	332.601	332.601	0.075412	0.0754382

177	59.47	-29.2328	20.0019	-0.0394307	0.94876	293.15	293.15	0	332.772	332.772	0.0754446	0.0754769

178	59.64	-32.8725	20.0008	-0.044338	0.974759	293.15	293.15	0	332.94	332.94	0.0754762	0.0755157

179	59.8	-36.8652	20.0008	-0.0497207	1.0008	293.15	293.15	0	333.104	333.104	0.0755083	0.0755538

180	59.97	-41.2668	20.0008	-0.0556544	1.02527	293.15	293.15	0	333.265	333.265	0.0755404	0.0755927

181	60.14	-45.8665	20.0008	-0.0618546	1.04992	293.15	293.15	0	333.425	333.425	0.0755738	0.0756326

182	60.31	-50.4094	20.0008	-0.0679775	1.07591	293.15	293.15	0	333.599	333.599	0.0756086	0.0756737

183	60.49	-54.7558	20.0008	-0.0738348	1.10001	293.15	293.15	0	333.766	333.766	0.0756447	0.0757151

184	60.68	-58.7601	20.0008	-0.0792297	1.11911	293.15	293.15	0	333.935	333.935	0.0756836	0.0757589

185	60.87	-62.4446	20.0008	-0.084193	1.13456	293.15	293.15	0	334.093	334.093	0.0757241	0.0758035

186	61.06	-65.7643	19.9956	-0.0886637	1.14761	293.15	293.15	0	334.258	334.258	0.0757649	0.0758481

187	61.25	-68.7313	20.0008	-0.0926584	1.15938	293.15	293.15	0	334.439	334.439	0.0758071	0.0758935

188	61.45	-71.2882	20.0008	-0.0960997	1.16902	293.15	293.15	0	334.595	334.595	0.0758509	0.0759396

189	61.64	-73.4821	20.0008	-0.0990514	1.17844	293.15	293.15	0	334.761	334.761	0.0758936	0.0759852

190	61.84	-75.3189	20.0008	-0.101521	1.18299	293.15	293.15	0	334.933	334.933	0.0759369	0.0760303

191	62.03	-76.7795	20.0008	-0.103484	1.1917	293.15	293.15	0	335.097	335.097	0.0759811	0.0760757

192	62.23	-77.9368	20.0008	-0.105038	1.19081	293.15	293.15	0	335.279	335.279	0.0760261	0.0761218

193	62.43	-78.7909	20.0008	-0.106182	1.18904	293.15	293.15	0	335.427	335.427	0.0760731	0.0761685

194	62.62	-79.3398	20.0008	-0.106916	1.19062	293.15	293.15	0	335.6	335.6	0.0761169	0.0762127

195	62.8	-79.5868	20.0008	-0.107243	1.1908	293.15	293.15	0	335.771	335.771	0.0761615	0.0762566

196	62.99	-79.5279	20.0008	-0.107157	1.19	293.15	293.15	0	335.937	335.937	0.0762063	0.0763011

197	63.18	-79.2481	20.0008	-0.106774	1.18823	293.15	293.15	0	336.11	336.11	0.0762506	0.0763449

198	63.37	-78.7858	20.0008	-0.106145	1.18555	293.15	293.15	0	336.273	336.273	0.0762946	0.0763876

199	63.54	-78.1878	20.0008	-0.105334	1.18494	293.15	293.15	0	336.431	336.431	0.0763377	0.0764292

200	63.72	-77.4531	19.9956	-0.104338	1.18381	293.15	293.15	0	336.604	336.604	0.0763799	0.0764706

201	63.9	-76.6146	20.0008	-0.103203	1.17967	293.15	293.15	0	336.768	336.768	0.0764229	0.0765123

202	64.07	-75.6386	20.0008	-0.101883	1.17611	293.15	293.15	0	336.938	336.938	0.0764651	0.0765526

203	64.25	-74.6079	20.0008	-0.10049	1.17901	293.15	293.15	0	337.089	337.089	0.0765062	0.0765933

204	64.42	-73.6983	20.0008	-0.0992594	1.17743	293.15	293.15	0	337.266	337.266	0.0765469	0.0766333

205	64.58	-72.9051	19.9956	-0.0981862	1.17803	293.15	293.15	0	337.436	337.436	0.0765866	0.0766721

206	64.75	-72.0624	20.0008	-0.0970464	1.17714	293.15	293.15	0	337.6	337.6	0.0766261	0.0767109

207	64.92	-71.0462	20.0008	-0.0956729	1.17462	293.15	293.15	0	337.773	337.773	0.0766679	0.0767512

208	65.09	-69.9706	19.9946	-0.0942197	1.17405	293.15	293.15	0	337.931	337.931	0.0767087	0.0767907

209	65.25	-68.8542	20.0008	-0.0927118	1.17292	293.15	293.15	0	338.094	338.094	0.0767485	0.0768283

210	65.42	-67.352	20.0008	-0.0906844	1.1638	293.15	293.15	0	338.269	338.269	0.0767917	0.0768677

211	65.59	-65.226	20.0008	-0.0878174	1.14909	293.15	293.15	0	338.44	338.44	0.0768365	0.0769079

212	65.77	-62.4296	20.0008	-0.084048	1.13806	293.15	293.15	0	338.606	338.606	0.076883	0.0769496

213	65.94	-59.3498	19.9904	-0.0798976	1.12529	293.15	293.15	0	338.761	338.761	0.0769273	0.0769897

214	66.11	-56.1222	19.9956	-0.0755486	1.1085	293.15	293.15	0	338.943	338.943	0.0769714	0.0770292

215	66.28	-52.6098	20.0008	-0.0708168	1.09296	293.15	293.15	0	339.108	339.108	0.0770161	0.0770683

216	66.44	-48.5525	19.9904	-0.0653522	1.07283	293.15	293.15	0	339.273	339.273	0.0770617	0.0771067

217	66.62	-43.8864	19.9946	-0.0590684	1.05287	293.15	293.15	0	339.436	339.436	0.07711	0.077147

218	66.79	-38.7629	20.0008	-0.0521699	1.02703	293.15	293.15	0	339.601	339.601	0.0771573	0.0771871

219	66.95	-33.4399	20.0008	-0.0450035	1.00374	293.15	293.15	0	339.775	339.775	0.0772034	0.0772254

220	67.11	-28.3217	20.0008	-0.0381137	0.988171	293.15	293.15	0	339.937	339.937	0.0772447	0.0772616

221	67.25	-23.7779	20.0008	-0.0319975	0.978379	293.15	293.15	0	340.095	340.095	0.0772829	0.0772954

222	67.39	-20.0042	20.0008	-0.0269181	0.973776	293.15	293.15	0	340.259	340.259	0.0773181	0.0773275

223	67.52	-16.9376	20.0008	-0.0227907	0.973046	293.15	293.15	0	340.433	340.433	0.0773511	0.0773579

224	67.65	-14.4708	20.0008	-0.0194707	0.975292	293.15	293.15	0	340.602	340.602	0.0773827	0.0773886

225	67.78	-12.5817	20.0008	-0.0169282	0.981151	293.15	293.15	0	340.77	340.77	0.0774143	0.0774193

226	67.91	-11.1854	20.0008	-0.015049	0.988673	293.15	293.15	0	340.94	340.94	0.0774456	0.07745

227	68.05	-10.1861	20.0008	-0.013704	0.995148	293.15	293.15	0	341.1	341.1	0.0774767	0.0774814

228	68.19	-9.53968	19.9956	-0.0128337	1.00285	293.15	293.15	0	341.273	341.273	0.0775094	0.0775135

229	68.33	-9.23006	20.0008	-0.0124167	1.01114	293.15	293.15	0	341.438	341.438	0.0775417	0.0775466

230	68.47	-9.02174	19.9998	-0.0121359	1.01858	293.15	293.15	0	341.596	341.596	0.0775755	0.0775799

231	68.62	-8.88546	19.9914	-0.011952	1.02487	293.15	293.15	0	341.767	341.767	0.0776101	0.0776151

232	68.77	-8.89833	20.0008	-0.0119688	1.03229	293.15	293.15	0	341.933	341.933	0.0776443	0.0776493

233	68.92	-9.01041	20.0008	-0.012119	1.04249	293.15	293.15	0	342.104	342.104	0.0776786	0.0776845

234	69.07	-9.16156	20.0008	-0.0123217	1.04798	293.15	293.15	0	342.27	342.27	0.0777147	0.0777207

235	69.23	-9.33414	20.0008	-0.0125533	1.05285	293.15	293.15	0	342.425	342.425	0.0777516	0.0777581

236	69.39	-9.48045	20.0008	-0.0127494	1.0595	293.15	293.15	0	342.609	342.609	0.077788	0.0777949

237	69.55	-9.54727	20.0008	-0.0128387	1.06587	293.15	293.15	0	342.765	342.765	0.0778244	0.0778312

238	69.71	-9.61266	20.0008	-0.012926	1.07473	293.15	293.15	0	342.936	342.936	0.0778613	0.0778692

239	69.88	-9.70552	20.0008	-0.0130502	1.08007	293.15	293.15	0	343.11	343.11	0.0778994	0.0779076

240	70.04	-9.77326	20.0008	-0.0131406	1.08419	293.15	293.15	0	343.273	343.273	0.077938	0.0779457

241	70.21	-9.89451	20.0008	-0.013303	1.08826	293.15	293.15	0	343.431	343.431	0.0779759	0.0779845

242	70.37	-10.028	20.0039	-0.0134818	1.0941	293.15	293.15	0	343.604	343.604	0.0780145	0.0780223

243	70.53	-10.0796	20.0112	-0.0135505	1.09903	293.15	293.15	0	343.768	343.768	0.0780531	0.078061

244	70.7	-10.1104	20.0112	-0.0135912	1.10396	293.15	293.15	0	343.929	343.929	0.0780907	0.0780992

245	70.87	-10.1474	20.0091	-0.0136402	1.10859	293.15	293.15	0	344.099	344.099	0.0781296	0.0781382

246	71.03	-10.1794	20.0008	-0.0136825	1.11171	293.15	293.15	0	344.267	344.267	0.0781695	0.0781774

247	71.2	-10.1877	20.0008	-0.0136931	1.12011	293.15	293.15	0	344.436	344.436	0.0782067	0.0782151

248	71.36	-10.1641	20.0008	-0.0136607	1.12474	293.15	293.15	0	344.603	344.603	0.0782459	0.0782543

249	71.53	-10.1084	20.0008	-0.0135852	1.12686	293.15	293.15	0	344.765	344.765	0.0782851	0.0782935

250	71.7	-10.156	20.0008	-0.0136484	1.13182	293.15	293.15	0	344.939	344.939	0.0783233	0.0783325

251	71.87	-10.2207	20.0008	-0.0137346	1.1376	293.15	293.15	0	345.103	345.103	0.0783624	0.0783713

252	72.03	-10.2707	20.0008	-0.0138011	1.14033	293.15	293.15	0	345.26	345.26	0.0784016	0.0784107

253	72.21	-10.3189	20.0008	-0.0138652	1.14305	293.15	293.15	0	345.432	345.432	0.0784404	0.0784504

254	72.37	-10.3863	20.0008	-0.013955	1.15068	293.15	293.15	0	345.597	345.597	0.0784795	0.0784892

255	72.54	-10.4549	20.006	-0.0140465	1.15526	293.15	293.15	0	345.771	345.771	0.0785177	0.0785279

256	72.71	-10.5166	20.0112	-0.0141287	1.15709	293.15	293.15	0	345.943	345.943	0.078557	0.0785676

257	72.88	-10.4989	20.0019	-0.0141042	1.16002	293.15	293.15	0	346.091	346.091	0.0785959	0.078607

258	73.04	-10.4362	20.0008	-0.0140192	1.16479	293.15	293.15	0	346.264	346.264	0.0786347	0.0786457

259	73.21	-10.4051	20.0008	-0.0139767	1.1715	293.15	293.15	0	346.435	346.435	0.0786733	0.0786844

260	73.38	-10.3338	20.0008	-0.0138802	1.17536	293.15	293.15	0	346.601	346.601	0.0787119	0.0787236

261	73.54	-10.241	20.0008	-0.0137549	1.1798	293.15	293.15	0	346.775	346.775	0.0787511	0.0787621

262	73.71	-10.1896	20.0008	-0.0136853	1.18655	293.15	293.15	0	346.946	346.946	0.0787898	0.0788012

263	73.88	-10.2136	20.0008	-0.0137167	1.19029	293.15	293.15	0	347.095	347.095	0.0788286	0.0788402

264	74.05	-10.3025	20.0029	-0.0138355	1.19355	293.15	293.15	0	347.269	347.269	0.0788674	0.0788794

265	74.21	-10.4043	19.9904	-0.0139714	1.19677	293.15	293.15	0	347.438	347.438	0.078906	0.0789181

266	74.38	-10.494	19.9987	-0.0140913	1.19955	293.15	293.15	0	347.606	347.606	0.0789452	0.0789573

267	74.55	-10.4813	19.9935	-0.0140735	1.20599	293.15	293.15	0	347.762	347.762	0.0789843	0.0789966

268	74.72	-10.4538	19.9904	-0.0140358	1.20967	293.15	293.15	0	347.93	347.93	0.0790232	0.079036

269	74.89	-10.3869	19.9977	-0.0139453	1.2153	293.15	293.15	0	348.1	348.1	0.0790615	0.0790744

270	75.05	-10.2894	20.0008	-0.0138137	1.22273	293.15	293.15	0	348.274	348.274	0.0790996	0.0791125

271	75.22	-10.2169	20.0008	-0.0137157	1.2269	293.15	293.15	0	348.44	348.44	0.0791385	0.079151

272	75.38	-10.2576	20.0008	-0.0137696	1.23039	293.15	293.15	0	348.612	348.612	0.0791771	0.0791903

273	75.55	-10.3223	20.0008	-0.0138557	1.23294	293.15	293.15	0	348.767	348.767	0.0792165	0.07923

274	75.72	-10.4077	20.0008	-0.0139696	1.23678	293.15	293.15	0	348.933	348.933	0.0792549	0.0792688

275	75.89	-10.4909	20.0008	-0.0140806	1.24196	293.15	293.15	0	349.097	349.097	0.0792942	0.0793084

276	76.06	-10.5857	20.0008	-0.0142071	1.24636	293.15	293.15	0	349.261	349.261	0.0793331	0.0793475

277	76.23	-10.6179	20.0008	-0.0142497	1.24812	293.15	293.15	0	349.443	349.443	0.0793719	0.0793862

278	76.39	-10.6178	20.0008	-0.0142488	1.25215	293.15	293.15	0	349.599	349.599	0.0794104	0.0794247

279	76.56	-10.5992	20.0008	-0.0142231	1.25625	293.15	293.15	0	349.765	349.765	0.0794491	0.0794635

280	76.73	-10.5082	20.0008	-0.0141003	1.26371	293.15	293.15	0	349.935	349.935	0.0794878	0.0795025

281	76.89	-10.4274	19.9914	-0.0139913	1.26743	293.15	293.15	0	350.101	350.101	0.0795262	0.0795406

282	77.06	-10.3253	19.9998	-0.0138535	1.27262	293.15	293.15	0	350.272	350.272	0.0795648	0.0795798

283	77.23	-10.2939	20.0008	-0.0138107	1.27784	293.15	293.15	0	350.431	350.431	0.0796037	0.0796189

284	77.39	-10.2516	20.0008	-0.0137532	1.28179	293.15	293.15	0	350.604	350.604	0.0796426	0.0796573

285	77.56	-10.2329	20.0008	-0.0137275	1.28631	293.15	293.15	0	350.769	350.769	0.0796814	0.0796964

286	77.72	-10.2537	20.0008	-0.0137547	1.29098	293.15	293.15	0	350.938	350.938	0.0797194	0.0797345

287	77.89	-10.3087	20.0008	-0.0138278	1.29821	293.15	293.15	0	351.096	351.096	0.079758	0.0797736

288	78.06	-10.3478	20.0008	-0.0138794	1.3009	293.15	293.15	0	351.266	351.266	0.0797973	0.0798129

289	78.23	-10.3217	20.0008	-0.0138438	1.30637	293.15	293.15	0	351.436	351.436	0.0798358	0.0798517

290	78.4	-10.2576	20.0008	-0.0137571	1.31203	293.15	293.15	0	351.609	351.609	0.0798743	0.0798903

291	78.56	-10.2178	20.0008	-0.013703	1.31501	293.15	293.15	0	351.773	351.773	0.0799131	0.0799296

292	78.73	-10.2132	20.0008	-0.0136962	1.32112	293.15	293.15	0	351.932	351.932	0.0799518	0.079968

293	78.89	-10.2049	20.0008	-0.0136844	1.32524	293.15	293.15	0	352.103	352.103	0.0799903	0.0800064

294	79.06	-10.2232	20.0008	-0.0137082	1.3292	293.15	293.15	0	352.269	352.269	0.0800294	0.0800457

295	79.23	-10.2667	20.0008	-0.0137659	1.33115	293.15	293.15	0	352.44	352.44	0.0800677	0.0800845

296	79.4	-10.3142	20.0008	-0.0138288	1.3394	293.15	293.15	0	352.606	352.606	0.0801066	0.0801239

297	79.56	-10.3289	20.0008	-0.0138478	1.34306	293.15	293.15	0	352.761	352.761	0.0801449	0.0801619

298	79.73	-10.311	19.9904	-0.0138232	1.3474	293.15	293.15	0	352.934	352.934	0.0801832	0.0802009

299	79.9	-10.2914	20.0008	-0.0137962	1.34921	293.15	293.15	0	353.098	353.098	0.0802227	0.0802404

300	80.07	-10.2913	20.0008	-0.0137954	1.35462	293.15	293.15	0	353.28	353.28	0.0802618	0.0802794

301	80.24	-10.277	20.0008	-0.0137755	1.35976	293.15	293.15	0	353.437	353.437	0.0803008	0.0803185

302	80.41	-10.2971	20.0008	-0.0138018	1.36539	293.15	293.15	0	353.603	353.603	0.0803388	0.0803571

303	80.57	-10.3089	20.0008	-0.0138168	1.36729	293.15	293.15	0	353.759	353.759	0.0803784	0.0803965

304	80.74	-10.3131	20.0008	-0.0138219	1.37489	293.15	293.15	0	353.928	353.928	0.0804164	0.0804347

305	80.91	-10.2573	20.0008	-0.0137463	1.37989	293.15	293.15	0	354.104	354.104	0.0804545	0.0804738

306	81.07	-10.2893	20.0008	-0.0137886	1.38243	293.15	293.15	0	354.274	354.274	0.0804938	0.0805123

307	81.24	-10.3348	20.0008	-0.0138488	1.38654	293.15	293.15	0	354.441	354.441	0.0805322	0.0805514

308	81.41	-10.3864	20.0008	-0.0139173	1.39199	293.15	293.15	0	354.608	354.608	0.080571	0.0805899

309	81.58	-10.3777	20.0008	-0.0139049	1.39735	293.15	293.15	0	354.763	354.763	0.0806097	0.0806289

310	81.74	-10.3616	20.0008	-0.0138827	1.40216	293.15	293.15	0	354.931	354.931	0.0806478	0.0806671

311	81.91	-10.3556	20.0008	-0.0138738	1.40799	293.15	293.15	0	355.109	355.109	0.0806866	0.0807055

312	82.08	-10.3191	20.0008	-0.0138242	1.41084	293.15	293.15	0	355.268	355.268	0.0807258	0.0807448

313	82.24	-10.3008	20.0008	-0.0137991	1.41431	293.15	293.15	0	355.429	355.429	0.0807645	0.0807834

314	82.41	-10.2722	20.0008	-0.0137601	1.42098	293.15	293.15	0	355.605	355.605	0.0808033	0.0808218

315	82.57	-10.2069	20.0008	-0.013672	1.42515	293.15	293.15	0	355.776	355.776	0.0808408	0.0808599

316	82.74	-10.2094	20.0008	-0.0136745	1.42788	293.15	293.15	0	355.942	355.942	0.0808796	0.080899

317	82.91	-10.1538	20.0008	-0.0135994	1.43574	293.15	293.15	0	356.097	356.097	0.0809186	0.0809385

318	83.08	-10.1187	20.0008	-0.0135517	1.43912	293.15	293.15	0	356.271	356.271	0.080957	0.0809775

319	83.25	-10.1387	20.0008	-0.0135778	1.44074	293.15	293.15	0	356.443	356.443	0.0809965	0.0810163

320	83.41	-10.1528	20.0008	-0.013596	1.44502	293.15	293.15	0	356.599	356.599	0.0810347	0.0810548

321	83.58	-10.1195	20.0008	-0.0135508	1.45036	293.15	293.15	0	356.764	356.764	0.0810726	0.0810931

322	83.75	-10.1245	20.0008	-0.0135568	1.45813	293.15	293.15	0	356.936	356.936	0.0811119	0.0811325

323	83.91	-10.1714	20.0008	-0.0136188	1.46157	293.15	293.15	0	357.102	357.102	0.0811502	0.0811712

324	84.08	-10.1986	20.0102	-0.0136546	1.46829	293.15	293.15	0	357.272	357.272	0.0811882	0.0812101

325	84.25	-10.2236	19.9998	-0.0136875	1.47184	293.15	293.15	0	357.431	357.431	0.0812267	0.0812487

326	84.42	-10.2832	19.9904	-0.0137665	1.47764	293.15	293.15	0	357.595	357.595	0.0812655	0.0812877

327	84.58	-10.3464	19.9987	-0.0138504	1.48289	293.15	293.15	0	357.769	357.769	0.0813043	0.0813266

328	84.75	-10.3351	19.9977	-0.0138346	1.48614	293.15	293.15	0	357.939	357.939	0.081343	0.0813655

329	84.92	-10.3416	19.9904	-0.0138425	1.48957	293.15	293.15	0	358.106	358.106	0.0813816	0.0814039

330	85.09	-10.3274	19.9987	-0.0138228	1.49576	293.15	293.15	0	358.271	358.271	0.0814208	0.0814428

331	85.25	-10.285	20.006	-0.0137655	1.49915	293.15	293.15	0	358.426	358.426	0.0814596	0.0814815

332	85.42	-10.2479	20.0008	-0.0137152	1.50537	293.15	293.15	0	358.594	358.594	0.081497	0.08152

333	85.59	-10.1862	19.9956	-0.0136318	1.51023	293.15	293.15	0	358.773	358.773	0.0815367	0.0815594

334	85.76	-10.1909	19.9998	-0.0136375	1.5146	293.15	293.15	0	358.932	358.932	0.0815753	0.0815978

335	85.92	-10.1931	19.9904	-0.0136398	1.52319	293.15	293.15	0	359.103	359.103	0.0816125	0.0816356

336	86.09	-10.1665	20.0019	-0.0136035	1.52484	293.15	293.15	0	359.269	359.269	0.0816517	0.0816754

337	86.26	-10.1873	20.0008	-0.0136305	1.52771	293.15	293.15	0	359.424	359.424	0.0816909	0.0817141

338	86.42	-10.2106	20.0008	-0.013661	1.53562	293.15	293.15	0	359.597	359.597	0.0817292	0.0817523

339	86.6	-10.2266	19.9904	-0.0136817	1.53773	293.15	293.15	0	359.77	359.77	0.0817683	0.0817926

340	86.76	-10.2714	20.0112	-0.013741	1.54172	293.15	293.15	0	359.944	359.944	0.0818068	0.081831

341	86.93	-10.2259	20.0019	-0.0136794	1.54504	293.15	293.15	0	360.091	360.091	0.0818454	0.0818688

342	87.09	-10.1279	20.0008	-0.0135476	1.55207	293.15	293.15	0	360.265	360.265	0.081883	0.0819069

343	87.26	-10.0786	20.0008	-0.0134811	1.55998	293.15	293.15	0	360.436	360.436	0.0819213	0.0819459

344	87.43	-10.129	20.0008	-0.0135479	1.56331	293.15	293.15	0	360.601	360.601	0.0819598	0.0819852

345	87.6	-10.1935	20.0008	-0.0136334	1.56684	293.15	293.15	0	360.774	360.774	0.0819994	0.0820246

346	87.77	-10.261	20.0008	-0.013723	1.5741	293.15	293.15	0	360.937	360.937	0.0820379	0.0820632

347	87.93	-10.2695	20.0008	-0.0137337	1.57873	293.15	293.15	0	361.095	361.095	0.0820762	0.0821011

348	88.1	-10.2591	20.0008	-0.013719	1.58239	293.15	293.15	0	361.268	361.268	0.0821147	0.0821398

349	88.26	-10.1911	20.0008	-0.0136275	1.58585	293.15	293.15	0	361.433	361.433	0.0821537	0.0821781

350	88.43	-10.1523	19.9987	-0.0135749	1.59053	293.15	293.15	0	361.602	361.602	0.0821916	0.0822165

351	88.6	-10.1574	20.0112	-0.013581	1.59686	293.15	293.15	0	361.763	361.763	0.0822297	0.082256

352	88.76	-10.2188	20.0112	-0.0136625	1.60338	293.15	293.15	0	361.93	361.93	0.0822681	0.0822943

353	88.93	-10.324	20.0039	-0.0138024	1.6106	293.15	293.15	0	362.109	362.109	0.0823065	0.0823334

354	89.1	-10.4003	20.0008	-0.0139037	1.61365	293.15	293.15	0	362.268	362.268	0.0823455	0.0823725

355	89.27	-10.4137	20.0008	-0.0139209	1.61728	293.15	293.15	0	362.429	362.429	0.0823842	0.0824111

356	89.44	-10.4407	20.0019	-0.0139562	1.62262	293.15	293.15	0	362.604	362.604	0.0824233	0.08245

357	89.61	-10.4619	20.0112	-0.0139839	1.62444	293.15	293.15	0	362.778	362.778	0.0824625	0.082489

358	89.77	-10.4627	19.9956	-0.0139843	1.62947	293.15	293.15	0	362.933	362.933	0.0825006	0.0825275

359	89.94	-10.3881	19.9904	-0.013884	1.63733	293.15	293.15	0	363.107	363.107	0.082539	0.0825653

360	90.1	-10.2388	20.0008	-0.0136837	1.64073	293.15	293.15	0	363.271	363.271	0.0825774	0.0826042

361	90.27	-10.1455	19.9956	-0.0135583	1.64724	293.15	293.15	0	363.436	363.436	0.0826152	0.0826423

362	90.44	-10.1341	20.0008	-0.0135424	1.6516	293.15	293.15	0	363.607	363.607	0.082654	0.0826814

363	90.6	-10.1429	20.0008	-0.0135535	1.65547	293.15	293.15	0	363.757	363.757	0.0826924	0.0827201

364	90.77	-10.1602	19.9977	-0.0135759	1.65927	293.15	293.15	0	363.936	363.936	0.0827311	0.0827591

365	90.94	-10.1703	19.9904	-0.0135887	1.6674	293.15	293.15	0	364.103	364.103	0.0827694	0.0827977

366	91.1	-10.1873	19.9987	-0.0136107	1.67186	293.15	293.15	0	364.276	364.276	0.0828076	0.0828356

367	91.27	-10.2429	20.0008	-0.0136843	1.67574	293.15	293.15	0	364.441	364.441	0.0828462	0.0828747

368	91.44	-10.2866	20.0008	-0.0137421	1.67969	293.15	293.15	0	364.601	364.601	0.0828847	0.0829129

369	91.61	-10.2871	20.0008	-0.013742	1.6831	293.15	293.15	0	364.762	364.762	0.0829242	0.0829524

370	91.77	-10.2448	19.9956	-0.0136849	1.69252	293.15	293.15	0	364.938	364.938	0.0829619	0.0829905

371	91.94	-10.169	20.0008	-0.0135829	1.69628	293.15	293.15	0	365.091	365.091	0.083001	0.0830293

372	92.11	-10.139	19.9956	-0.0135421	1.7008	293.15	293.15	0	365.264	365.264	0.083039	0.0830678

373	92.28	-10.1129	19.9998	-0.0135065	1.70956	293.15	293.15	0	365.43	365.43	0.0830771	0.0831062

374	92.44	-10.154	19.9914	-0.0135608	1.71313	293.15	293.15	0	365.602	365.602	0.0831156	0.083145

375	92.61	-10.1856	20.0008	-0.0136023	1.71576	293.15	293.15	0	365.774	365.774	0.0831547	0.0831842

376	92.78	-10.1529	20.0008	-0.0135579	1.71979	293.15	293.15	0	365.932	365.932	0.0831931	0.0832222

377	92.94	-10.0983	20.0008	-0.0134844	1.72729	293.15	293.15	0	366.095	366.095	0.0832315	0.0832609

378	93.11	-10.0374	20.0008	-0.0134024	1.73056	293.15	293.15	0	366.269	366.269	0.0832701	0.0832991

379	93.28	-10.0035	20.0008	-0.0133564	1.73734	293.15	293.15	0	366.426	366.426	0.0833079	0.0833377

380	93.45	-10.0429	20.0008	-0.0134084	1.74054	293.15	293.15	0	366.598	366.598	0.0833467	0.0833764

381	93.62	-10.1079	20.0008	-0.0134945	1.74688	293.15	293.15	0	366.772	366.772	0.0833855	0.083416

382	93.78	-10.1377	20.0008	-0.0135335	1.75375	293.15	293.15	0	366.943	366.943	0.0834231	0.0834542

383	93.95	-10.1828	20.0008	-0.0135931	1.75847	293.15	293.15	0	367.102	367.102	0.0834614	0.0834928

384	94.12	-10.1943	20.0008	-0.0136077	1.76083	293.15	293.15	0	367.266	367.266	0.0835007	0.0835316

385	94.29	-10.27	20.0008	-0.0137082	1.76392	293.15	293.15	0	367.436	367.436	0.0835396	0.0835706

386	94.45	-10.3052	20.0008	-0.0137544	1.77098	293.15	293.15	0	367.603	367.603	0.0835783	0.0836088

387	94.62	-10.256	19.9977	-0.0136881	1.77582	293.15	293.15	0	367.776	367.776	0.0836163	0.0836473

388	94.79	-10.1735	19.9904	-0.0135772	1.78087	293.15	293.15	0	367.937	367.937	0.0836548	0.0836858

389	94.95	-10.0262	19.9977	-0.01338	1.78587	293.15	293.15	0	368.097	368.097	0.0836929	0.0837239

390	95.12	-9.95593	20.0008	-0.0132856	1.7951	293.15	293.15	0	368.27	368.27	0.0837308	0.0837627

391	95.28	-10.053	20.0008	-0.0134144	1.80007	293.15	293.15	0	368.434	368.434	0.0837683	0.0838011

392	95.45	-10.0926	20.0008	-0.0134666	1.80442	293.15	293.15	0	368.602	368.602	0.0838072	0.0838396

393	95.62	-10.1435	20.0008	-0.0135338	1.81083	293.15	293.15	0	368.772	368.772	0.0838464	0.0838795

394	95.79	-10.2213	20.0008	-0.0136369	1.8158	293.15	293.15	0	368.938	368.938	0.0838851	0.0839182

395	95.96	-10.2922	20.0008	-0.013731	1.81957	293.15	293.15	0	369.094	369.094	0.0839239	0.0839567

396	96.13	-10.3848	20.0008	-0.0138537	1.82466	293.15	293.15	0	369.266	369.266	0.0839617	0.0839951

397	96.29	-10.4351	20.0008	-0.0139202	1.82894	293.15	293.15	0	369.439	369.439	0.0839998	0.0840336

398	96.46	-10.4308	20.0008	-0.0139136	1.83455	293.15	293.15	0	369.605	369.605	0.0840387	0.0840724

399	96.63	-10.3704	20.0008	-0.0138325	1.83941	293.15	293.15	0	369.761	369.761	0.0840773	0.0841107

400	96.79	-10.3416	20.0008	-0.0137933	1.84295	293.15	293.15	0	369.933	369.933	0.0841153	0.0841488

401	96.96	-10.3552	20.0008	-0.0138108	1.85202	293.15	293.15	0	370.107	370.107	0.0841533	0.0841873

402	97.13	-10.3268	20.0008	-0.0137722	1.85352	293.15	293.15	0	370.27	370.27	0.0841923	0.0842262

403	97.29	-10.3192	19.9966	-0.0137614	1.85805	293.15	293.15	0	370.427	370.427	0.0842309	0.0842647

404	97.46	-10.3275	19.9904	-0.0137718	1.86449	293.15	293.15	0	370.607	370.607	0.0842692	0.0843036

405	97.63	-10.2703	19.9904	-0.0136948	1.87061	293.15	293.15	0	370.773	370.773	0.0843073	0.0843418

406	97.8	-10.2048	19.9998	-0.0136068	1.87779	293.15	293.15	0	370.939	370.939	0.0843455	0.0843803

407	97.96	-10.1666	20.0008	-0.0135552	1.88085	293.15	293.15	0	371.094	371.094	0.0843847	0.0844188

408	98.13	-10.1417	20.0008	-0.0135212	1.88449	293.15	293.15	0	371.264	371.264	0.0844233	0.0844578

409	98.3	-10.1413	20.0008	-0.0135201	1.89127	293.15	293.15	0	371.431	371.431	0.0844615	0.0844968

410	98.47	-10.1638	20.0008	-0.0135495	1.89612	293.15	293.15	0	371.6	371.6	0.0844998	0.0845354

411	98.63	-10.1387	20.0008	-0.0135153	1.90295	293.15	293.15	0	371.77	371.77	0.084538	0.0845729

412	98.8	-10.1023	20.0008	-0.0134661	1.9084	293.15	293.15	0	371.938	371.938	0.0845759	0.0846116

413	98.97	-10.1533	20.0008	-0.0135333	1.91312	293.15	293.15	0	372.108	372.108	0.0846148	0.0846504

414	99.14	-10.2141	19.9935	-0.0136137	1.91905	293.15	293.15	0	372.263	372.263	0.0846532	0.0846897

415	99.3	-10.2447	19.9914	-0.0136539	1.92521	293.15	293.15	0	372.428	372.428	0.0846912	0.0847277

416	99.47	-10.2723	20.0008	-0.0136899	1.92866	293.15	293.15	0	372.595	372.595	0.0847298	0.0847663

417	99.63	-10.236	20.006	-0.0136409	1.93314	293.15	293.15	0	372.775	372.775	0.0847679	0.0848041

418	99.8	-10.216	20.0008	-0.0136136	1.93759	293.15	293.15	0	372.931	372.931	0.0848063	0.0848427

419	99.97	-10.2552	20.0008	-0.0136651	1.94555	293.15	293.15	0	373.095	373.095	0.0848444	0.084881

420	100.13	-10.3224	20.0008	-0.0137539	1.85904	293.15	293.15	0	373.05	373.05	0.0848825	0.0849192

421	100.26	-10.3178	20.0008	-0.0137473	1.7345	293.15	293.15	0	372.886	372.886	0.0849121	0.0849485

422	100.31	-9.91245	20.0112	-0.013207	1.61569	293.15	293.15	0	372.704	372.704	0.0849259	0.0849598

423	100.28	-8.52216	20.0019	-0.0113548	1.5352	293.15	293.15	0	372.557	372.557	0.0849243	0.084953

424	100.2	-6.23505	20.0008	-0.00830767	1.4563	293.15	293.15	0	372.383	372.383	0.0849099	0.0849338

425	100.06	-3.38744	20.0008	-0.00451366	1.39835	293.15	293.15	0	372.218	372.218	0.0848844	0.0849031

426	99.9	-0.295342	20.0008	-0.000393553	1.35003	293.15	293.15	0	372.046	372.046	0.0848507	0.0848647

427	99.7	2.76575	20.0008	0.00368566	1.31789	293.15	293.15	0	371.889	371.889	0.0848094	0.08482

428	99.49	5.65167	20.0008	0.00753196	1.28557	293.15	293.15	0	371.711	371.711	0.0847643	0.0847709

429	99.27	8.24357	20.0008	0.0109869	1.26845	293.15	293.15	0	371.56	371.56	0.0847161	0.0847203

430	99.04	10.47	20.0008	0.0139553	1.25291	293.15	293.15	0	371.391	371.391	0.084666	0.0846669

431	98.8	12.329	20.0008	0.0164342	1.24398	293.15	293.15	0	371.222	371.222	0.084613	0.0846127

432	98.57	13.8519	20.0008	0.0184654	1.23631	293.15	293.15	0	371.045	371.045	0.0845595	0.0845583

433	98.34	15.0043	20.0008	0.0200031	1.23179	293.15	293.15	0	370.875	370.875	0.0845069	0.0845053

434	98.11	15.8159	20.0008	0.0210865	1.23214	293.15	293.15	0	370.728	370.728	0.0844551	0.0844524

435	97.88	16.4091	20.0008	0.0218788	1.23577	293.15	293.15	0	370.555	370.555	0.0844035	0.0844001

436	97.65	16.824	20.0008	0.0224335	1.23551	293.15	293.15	0	370.388	370.388	0.0843511	0.0843478

437	97.44	16.97	20.0008	0.0226297	1.23891	293.15	293.15	0	370.225	370.225	0.0843017	0.0842986

438	97.23	16.9129	20.0112	0.022555	1.24421	293.15	293.15	0	370.052	370.052	0.0842527	0.0842498

439	97.03	16.7645	20.0008	0.0223585	1.24691	293.15	293.15	0	369.878	369.878	0.084206	0.0842027

440	96.83	16.5433	20.0008	0.0220649	1.24528	293.15	293.15	0	369.724	369.724	0.0841596	0.0841566

441	96.63	16.2449	20.0008	0.021668	1.24739	293.15	293.15	0	369.558	369.558	0.0841148	0.0841116

442	96.44	15.9706	20.0008	0.0213035	1.24706	293.15	293.15	0	369.377	369.377	0.0840701	0.0840672

443	96.25	15.7467	20.0008	0.0210059	1.24801	293.15	293.15	0	369.227	369.227	0.0840267	0.0840241

444	96.07	15.5015	20.0008	0.02068	1.24733	293.15	293.15	0	369.058	369.058	0.0839841	0.0839817

445	95.89	15.2485	20.0008	0.0203436	1.2455	293.15	293.15	0	368.882	368.882	0.0839423	0.0839399

446	95.71	14.9536	20.0008	0.0199511	1.24539	293.15	293.15	0	368.712	368.712	0.0839011	0.083899

447	95.54	14.6512	20.0008	0.0195488	1.24569	293.15	293.15	0	368.561	368.561	0.0838608	0.0838594

448	95.36	14.3614	20.0008	0.0191631	1.24107	293.15	293.15	0	368.384	368.384	0.0838209	0.0838191

449	95.19	14.1808	20.0008	0.018923	1.23666	293.15	293.15	0	368.214	368.214	0.083781	0.0837792

450	95.02	14.0281	19.9956	0.0187202	1.23482	293.15	293.15	0	368.05	368.05	0.0837411	0.0837392

451	94.85	13.8693	20.0008	0.0185092	1.22979	293.15	293.15	0	367.894	367.894	0.0837027	0.0837011

452	94.69	13.7206	20.0008	0.0183118	1.22702	293.15	293.15	0	367.728	367.728	0.0836639	0.0836627

453	94.52	13.5563	20.0008	0.0180933	1.22426	293.15	293.15	0	367.547	367.547	0.0836253	0.083624

454	94.35	13.3967	20.0008	0.0178812	1.2199	293.15	293.15	0	367.39	367.39	0.083586	0.0835844

455	94.18	13.283	20.0008	0.0177305	1.21764	293.15	293.15	0	367.226	367.226	0.0835466	0.0835454

456	94.01	13.2615	19.9904	0.0177026	1.21419	293.15	293.15	0	367.053	367.053	0.0835089	0.0835072

457	93.85	13.2165	20.0008	0.0176434	1.20463	293.15	293.15	0	366.88	366.88	0.0834713	0.0834695

458	93.68	13.1822	20.0008	0.0175984	1.20045	293.15	293.15	0	366.716	366.716	0.0834339	0.0834317

459	93.51	13.1714	20.0008	0.0175849	1.19737	293.15	293.15	0	366.559	366.559	0.083395	0.0833924

460	93.35	13.1588	19.9914	0.017569	1.19053	293.15	293.15	0	366.378	366.378	0.0833567	0.0833546

461	93.18	13.1214	19.9987	0.0175199	1.18768	293.15	293.15	0	366.229	366.229	0.0833182	0.0833158

462	93.01	13.0968	20.0008	0.0174879	1.18121	293.15	293.15	0	366.051	366.051	0.0832792	0.0832768

463	92.85	13.0496	20.0008	0.0174257	1.17711	293.15	293.15	0	365.883	365.883	0.0832413	0.0832386

464	92.68	13.0062	20.0008	0.0173687	1.17272	293.15	293.15	0	365.717	365.717	0.0832031	0.0832001

465	92.51	12.9958	20.0008	0.0173557	1.167	293.15	293.15	0	365.562	365.562	0.0831646	0.0831614

466	92.35	13.0357	20.0008	0.0174098	1.16127	293.15	293.15	0	365.394	365.394	0.0831262	0.0831228

467	92.18	13.0472	20.0008	0.017426	1.15466	293.15	293.15	0	365.216	365.216	0.0830884	0.0830843

468	92.01	13.1263	20.0008	0.0175326	1.15164	293.15	293.15	0	365.048	365.048	0.0830493	0.0830456

469	91.84	13.2194	20.0008	0.0176579	1.14613	293.15	293.15	0	364.878	364.878	0.0830109	0.0830062

470	91.68	13.2438	20.0008	0.0176913	1.14445	293.15	293.15	0	364.712	364.712	0.0829721	0.0829681

471	91.5	13.2607	20.0008	0.0177148	1.13674	293.15	293.15	0	364.557	364.557	0.0829331	0.0829282

472	91.34	13.3381	20.0008	0.0178191	1.13214	293.15	293.15	0	364.392	364.392	0.0828955	0.0828908

473	91.18	13.3604	19.9998	0.0178498	1.12898	293.15	293.15	0	364.211	364.211	0.0828572	0.0828527

474	91.01	13.2907	19.9904	0.0177576	1.12611	293.15	293.15	0	364.054	364.054	0.0828183	0.0828136

475	90.84	13.222	20.0008	0.0176666	1.11824	293.15	293.15	0	363.89	363.89	0.08278	0.0827752

476	90.67	13.2116	20.0008	0.0176537	1.11453	293.15	293.15	0	363.716	363.716	0.0827416	0.0827363

477	90.51	13.2226	20.0008	0.0176692	1.11097	293.15	293.15	0	363.544	363.544	0.0827031	0.0826981

478	90.34	13.2118	20.0008	0.0176557	1.10524	293.15	293.15	0	363.379	363.379	0.0826647	0.0826593

479	90.17	13.1813	20.0008	0.0176158	1.10034	293.15	293.15	0	363.214	363.214	0.0826255	0.0826204

480	90	13.1889	20.0008	0.0176269	1.09552	293.15	293.15	0	363.041	363.041	0.0825865	0.0825813

481	89.84	13.2231	20.0008	0.0176734	1.09108	293.15	293.15	0	362.884	362.884	0.0825485	0.0825431

482	89.67	13.208	20.0008	0.0176541	1.08673	293.15	293.15	0	362.714	362.714	0.0825101	0.0825045

483	89.51	13.172	20.0008	0.0176069	1.07939	293.15	293.15	0	362.559	362.559	0.0824713	0.0824659

484	89.34	13.1582	20.0008	0.0175893	1.07799	293.15	293.15	0	362.379	362.379	0.0824328	0.0824268

485	89.17	13.1675	20.0008	0.0176027	1.07089	293.15	293.15	0	362.224	362.224	0.0823938	0.0823877

486	89	13.1873	20.0008	0.01763	1.06703	293.15	293.15	0	362.058	362.058	0.0823555	0.0823491

487	88.83	13.2182	20.0008	0.0176722	1.06423	293.15	293.15	0	361.877	361.877	0.0823165	0.08231

488	88.67	13.1947	20.0008	0.0176417	1.05972	293.15	293.15	0	361.721	361.721	0.082278	0.0822716

489	88.5	13.1655	20.0008	0.0176035	1.05331	293.15	293.15	0	361.557	361.557	0.0822397	0.0822326

490	88.33	13.1357	20.0008	0.0175646	1.05092	293.15	293.15	0	361.384	361.384	0.0822008	0.082193

491	88.16	13.085	20.0008	0.0174976	1.04724	293.15	293.15	0	361.22	361.22	0.0821623	0.0821547

492	87.99	13.037	20.0008	0.0174343	1.04157	293.15	293.15	0	361.046	361.046	0.0821238	0.0821164

493	87.83	13.0549	20.0008	0.0174591	1.03676	293.15	293.15	0	360.89	360.89	0.0820857	0.0820783

494	87.66	13.106	20.0008	0.0175284	1.03148	293.15	293.15	0	360.716	360.716	0.0820467	0.0820393

495	87.49	13.0996	20.0008	0.0175208	1.02877	293.15	293.15	0	360.552	360.552	0.0820079	0.0820002

496	87.32	13.0921	20.0008	0.0175116	1.0239	293.15	293.15	0	360.38	360.38	0.0819692	0.081961

497	87.15	13.0762	20.0008	0.0174911	1.0176	293.15	293.15	0	360.215	360.215	0.0819308	0.0819214

498	86.99	13.0882	20.0008	0.0175081	1.01146	293.15	293.15	0	360.044	360.044	0.0818927	0.0818828

499	86.82	13.0844	20.0008	0.0175039	1.00909	293.15	293.15	0	359.885	359.885	0.0818539	0.0818451

500	86.66	13.0831	19.9977	0.017503	1.00383	293.15	293.15	0	359.721	359.721	0.081816	0.081807

501	86.48	13.1737	19.9935	0.0176252	0.99826	293.15	293.15	0	359.548	359.548	0.0817771	0.0817667

502	86.32	13.3022	20.0008	0.017798	0.99572	293.15	293.15	0	359.387	359.387	0.0817377	0.0817282

503	86.15	13.3803	20.0008	0.0179034	0.991969	293.15	293.15	0	359.228	359.228	0.0816991	0.0816893

504	85.98	13.3651	20.0008	0.0178839	0.985435	293.15	293.15	0	359.05	359.05	0.0816607	0.0816509

505	85.82	13.2972	20.0008	0.0177939	0.980167	293.15	293.15	0	358.881	358.881	0.0816217	0.0816126

506	85.65	13.2495	20.0008	0.017731	0.974735	293.15	293.15	0	358.715	358.715	0.0815831	0.0815733

507	85.48	13.2765	20.0008	0.0177681	0.972428	293.15	293.15	0	358.56	358.56	0.0815438	0.0815336

508	85.31	13.3145	20.0008	0.0178199	0.970193	293.15	293.15	0	358.394	358.394	0.0815048	0.0814944

509	85.14	13.2613	20.0008	0.0177495	0.966495	293.15	293.15	0	358.214	358.214	0.0814664	0.0814556

510	84.98	13.2083	19.9998	0.0176794	0.959486	293.15	293.15	0	358.048	358.048	0.0814278	0.0814179

511	84.81	13.1405	19.9904	0.0175896	0.955512	293.15	293.15	0	357.892	357.892	0.0813894	0.0813795

512	84.65	13.1212	19.9956	0.0175646	0.951133	293.15	293.15	0	357.719	357.719	0.0813516	0.0813413

513	84.48	13.1367	20.0008	0.0175863	0.943616	293.15	293.15	0	357.555	357.555	0.0813132	0.0813029

514	84.31	13.1929	20.0008	0.0176624	0.941724	293.15	293.15	0	357.383	357.383	0.0812744	0.081263

515	84.14	13.2767	20.0008	0.0177755	0.940662	293.15	293.15	0	357.226	357.226	0.0812346	0.0812235

516	83.97	13.3333	20.0008	0.0178522	0.93389	293.15	293.15	0	357.045	357.045	0.0811961	0.0811843

517	83.81	13.3575	19.9966	0.0178854	0.929243	293.15	293.15	0	356.88	356.88	0.0811584	0.0811463

518	83.64	13.3276	19.9904	0.0178464	0.924927	293.15	293.15	0	356.724	356.724	0.0811189	0.0811071

519	83.47	13.3032	20.0071	0.0178145	0.919198	293.15	293.15	0	356.558	356.558	0.0810806	0.0810685

520	83.3	13.3132	19.9998	0.0178288	0.915889	293.15	293.15	0	356.389	356.389	0.0810422	0.0810297

521	83.14	13.2579	19.9904	0.0177556	0.913518	293.15	293.15	0	356.221	356.221	0.0810027	0.0809909

522	82.97	13.188	19.9987	0.0176629	0.908037	293.15	293.15	0	356.043	356.043	0.0809644	0.0809522

523	82.8	13.1215	20.0008	0.0175748	0.902304	293.15	293.15	0	355.875	355.875	0.0809258	0.0809139

524	82.64	13.0357	20.0008	0.0174607	0.900586	293.15	293.15	0	355.72	355.72	0.080887	0.0808752

525	82.47	12.9813	20.0008	0.0173887	0.892955	293.15	293.15	0	355.549	355.549	0.0808488	0.0808368

526	82.3	12.954	20.0008	0.017353	0.889649	293.15	293.15	0	355.379	355.379	0.0808101	0.0807973

527	82.14	13.0254	20.0008	0.0174495	0.881261	293.15	293.15	0	355.224	355.224	0.0807718	0.0807586

528	81.97	13.1106	19.9998	0.0175645	0.879372	293.15	293.15	0	355.058	355.058	0.0807325	0.0807195

529	81.8	13.2002	19.9914	0.0176854	0.875976	293.15	293.15	0	354.887	354.887	0.0806937	0.0806807

530	81.63	13.2561	20.0008	0.0177613	0.872637	293.15	293.15	0	354.714	354.714	0.0806549	0.0806417

531	81.46	13.2835	20.0008	0.0177989	0.865565	293.15	293.15	0	354.548	354.548	0.0806167	0.0806026

532	81.29	13.2413	20.0008	0.0177432	0.862868	293.15	293.15	0	354.385	354.385	0.0805781	0.0805634

533	81.13	13.2276	20.0008	0.0177257	0.860986	293.15	293.15	0	354.22	354.22	0.0805387	0.0805246

534	80.96	13.2774	20.0008	0.0177934	0.853375	293.15	293.15	0	354.056	354.056	0.0805003	0.080486

535	80.79	13.2861	20.0008	0.017806	0.850245	293.15	293.15	0	353.882	353.882	0.0804612	0.0804468

536	80.62	13.2471	19.9904	0.0177546	0.850314	293.15	293.15	0	353.719	353.719	0.0804216	0.0804075

537	80.46	13.2439	19.9998	0.0177512	0.842391	293.15	293.15	0	353.552	353.552	0.0803845	0.0803698

538	80.29	13.2436	20.0008	0.0177517	0.839483	293.15	293.15	0	353.381	353.381	0.0803454	0.0803301

539	80.12	13.2508	20.0008	0.0177622	0.833441	293.15	293.15	0	353.215	353.215	0.0803062	0.0802913

540	79.96	13.2141	20.0008	0.0177139	0.828608	293.15	293.15	0	353.051	353.051	0.0802674	0.0802529

541	79.79	13.1253	20.0091	0.0175958	0.826783	293.15	293.15	0	352.894	352.894	0.0802282	0.0802134

542	79.62	13.0774	20.0029	0.0175325	0.823271	293.15	293.15	0	352.725	352.725	0.0801899	0.0801739

543	79.45	13.0898	20.0008	0.01755	0.818856	293.15	293.15	0	352.548	352.548	0.0801509	0.0801352

544	79.28	13.1256	20.0008	0.0175988	0.812332	293.15	293.15	0	352.388	352.388	0.0801133	0.080097

545	79.12	13.1778	20.0008	0.0176697	0.80649	293.15	293.15	0	352.214	352.214	0.0800748	0.0800587

546	78.95	13.2565	20.0008	0.0177762	0.804669	293.15	293.15	0	352.054	352.054	0.0800351	0.0800191

547	78.79	13.317	20.0008	0.0178581	0.799454	293.15	293.15	0	351.888	351.888	0.0799975	0.0799816

548	78.62	13.34	20.0008	0.0178899	0.793604	293.15	293.15	0	351.723	351.723	0.079958	0.079942

549	78.45	13.3106	20.0008	0.0178514	0.790255	293.15	293.15	0	351.558	351.558	0.0799195	0.0799031

550	78.28	13.3265	20.0008	0.0178737	0.789925	293.15	293.15	0	351.376	351.376	0.0798797	0.0798631

551	78.12	13.2956	20.0008	0.017833	0.785447	293.15	293.15	0	351.211	351.211	0.0798415	0.0798253

552	77.95	13.3323	20.0008	0.0178832	0.777699	293.15	293.15	0	351.057	351.057	0.0798029	0.0797859

553	77.78	13.3318	20.006	0.0178834	0.776177	293.15	293.15	0	350.891	350.891	0.0797638	0.0797476

554	77.61	13.3374	20.0008	0.0178919	0.769837	293.15	293.15	0	350.711	350.711	0.0797254	0.079709

555	77.45	13.3159	20.0008	0.0178638	0.765998	293.15	293.15	0	350.556	350.556	0.0796877	0.0796706

556	77.28	13.2732	20.0008	0.0178075	0.760203	293.15	293.15	0	350.388	350.388	0.0796484	0.0796311

557	77.11	13.2419	20.0008	0.0177665	0.754749	293.15	293.15	0	350.215	350.215	0.0796099	0.0795919

558	76.95	13.2294	20.0008	0.0177505	0.753074	293.15	293.15	0	350.051	350.051	0.0795707	0.0795535

559	76.78	13.2137	20.0008	0.0177304	0.750194	293.15	293.15	0	349.881	349.881	0.0795317	0.079514

560	76.61	13.1973	20.0008	0.0177092	0.744196	293.15	293.15	0	349.708	349.708	0.0794927	0.079475

561	76.44	13.1854	20.0008	0.0176941	0.73991	293.15	293.15	0	349.546	349.546	0.0794545	0.0794364

562	76.27	13.2166	20.0008	0.017737	0.735582	293.15	293.15	0	349.384	349.384	0.0794155	0.0793966

563	76.1	13.2614	20.0008	0.017798	0.730398	293.15	293.15	0	349.21	349.21	0.0793766	0.0793579

564	75.94	13.3099	20.0008	0.0178639	0.727984	293.15	293.15	0	349.051	349.051	0.0793376	0.0793188

565	75.77	13.3173	20.0008	0.0178748	0.72531	293.15	293.15	0	348.89	348.89	0.0792985	0.0792797

566	75.6	13.3488	20.0008	0.017918	0.719619	293.15	293.15	0	348.715	348.715	0.0792596	0.0792407

567	75.43	13.3821	20.0019	0.0179636	0.716439	293.15	293.15	0	348.543	348.543	0.0792213	0.0792021

568	75.27	13.3134	20.0112	0.0178723	0.716098	293.15	293.15	0	348.377	348.377	0.0791814	0.0791627

569	75.1	13.1496	20.0112	0.0176534	0.709209	293.15	293.15	0	348.222	348.222	0.0791422	0.0791235

570	74.93	13.051	20.0008	0.0175218	0.705438	293.15	293.15	0	348.048	348.048	0.0791039	0.0790853

571	74.77	12.9803	20.0008	0.0174278	0.702447	293.15	293.15	0	347.876	347.876	0.0790655	0.0790465

572	74.6	12.9713	20.0008	0.0174166	0.700191	293.15	293.15	0	347.721	347.721	0.0790267	0.0790078

573	74.43	12.9832	20.0008	0.0174334	0.695859	293.15	293.15	0	347.555	347.555	0.0789881	0.078969

574	74.26	12.9766	20.0008	0.0174254	0.688941	293.15	293.15	0	347.384	347.384	0.0789492	0.0789298

575	74.1	12.9589	20.0008	0.0174025	0.683501	293.15	293.15	0	347.209	347.209	0.0789109	0.0788911

576	73.94	12.9168	20.0008	0.0173468	0.679301	293.15	293.15	0	347.047	347.047	0.0788728	0.0788536

577	73.77	12.9404	20.0008	0.0173794	0.675491	293.15	293.15	0	346.888	346.888	0.0788345	0.0788143

578	73.6	13.0181	20.0008	0.0174846	0.670946	293.15	293.15	0	346.715	346.715	0.0787951	0.0787747

579	73.43	13.0727	19.9977	0.0175589	0.666647	293.15	293.15	0	346.545	346.545	0.0787559	0.0787353

580	73.26	13.0641	19.9904	0.0175482	0.665392	293.15	293.15	0	346.386	346.386	0.0787171	0.0786968

581	73.09	13.0293	19.9977	0.0175024	0.660082	293.15	293.15	0	346.221	346.221	0.0786778	0.0786566

582	72.92	13.0263	20.0008	0.0174992	0.654209	293.15	293.15	0	346.053	346.053	0.0786392	0.0786177

583	72.75	13.0871	20.0008	0.0175818	0.648935	293.15	293.15	0	345.891	345.891	0.0786002	0.0785784

584	72.59	13.1342	20.0008	0.0176459	0.646333	293.15	293.15	0	345.725	345.725	0.0785616	0.0785399

585	72.42	13.2096	20.0008	0.0177482	0.643321	293.15	293.15	0	345.553	345.553	0.0785223	0.0785005

586	72.26	13.145	20.0008	0.0176623	0.639115	293.15	293.15	0	345.378	345.378	0.0784845	0.078463

587	72.09	13.0778	19.9956	0.0175729	0.633052	293.15	293.15	0	345.223	345.223	0.0784455	0.0784242

588	71.93	13.0474	20.0008	0.0175329	0.629606	293.15	293.15	0	345.05	345.05	0.0784066	0.0783851

589	71.76	13.0352	20.0008	0.0175174	0.628766	293.15	293.15	0	344.878	344.878	0.0783674	0.0783463

590	71.59	13.0295	20.0008	0.0175106	0.623585	293.15	293.15	0	344.713	344.713	0.0783282	0.0783068

591	71.42	12.9843	20.0008	0.0174507	0.619371	293.15	293.15	0	344.557	344.557	0.0782897	0.0782671

592	71.25	12.9386	20.0008	0.0173902	0.614462	293.15	293.15	0	344.383	344.383	0.0782507	0.0782279

593	71.08	12.9523	20.0008	0.0174095	0.612215	293.15	293.15	0	344.212	344.212	0.0782112	0.0781885

594	70.91	12.9798	20.0008	0.0174474	0.609122	293.15	293.15	0	344.045	344.045	0.0781726	0.0781497

595	70.75	13.0171	20.0008	0.0174984	0.600678	293.15	293.15	0	343.889	343.889	0.0781343	0.0781107

596	70.58	13.0559	20.0008	0.0175514	0.59805	293.15	293.15	0	343.719	343.719	0.0780952	0.0780716

597	70.41	13.1273	20.0008	0.0176484	0.595634	293.15	293.15	0	343.552	343.552	0.0780562	0.0780325

598	70.25	13.2127	20.0008	0.017764	0.592283	293.15	293.15	0	343.378	343.378	0.0780169	0.0779937

599	70.08	13.2381	20.0008	0.017799	0.587653	293.15	293.15	0	343.209	343.209	0.0779775	0.0779542

600	69.91	13.2558	20.0008	0.0178238	0.582986	293.15	293.15	0	343.045	343.045	0.0779387	0.0779144

601	69.74	13.1905	20.0008	0.0177369	0.578012	293.15	293.15	0	342.875	342.875	0.0779004	0.0778764

602	69.57	13.1384	20.0008	0.0176676	0.575065	293.15	293.15	0	342.71	342.71	0.0778619	0.0778374

603	69.41	13.0597	20.0008	0.0175627	0.572231	293.15	293.15	0	342.555	342.555	0.0778233	0.077799

604	69.24	13.0238	20.0019	0.0175154	0.565041	293.15	293.15	0	342.389	342.389	0.0777846	0.0777596

605	69.07	13.0606	20.0102	0.0175658	0.563658	293.15	293.15	0	342.216	342.216	0.0777449	0.0777198

606	68.9	13.1858	19.9956	0.0177351	0.563646	293.15	293.15	0	342.052	342.052	0.0777052	0.0776798

607	68.73	13.3038	19.9904	0.0178946	0.558441	293.15	293.15	0	341.888	341.888	0.0776665	0.0776415

608	68.57	13.2996	20.0008	0.0178899	0.553729	293.15	293.15	0	341.714	341.714	0.0776275	0.0776023

609	68.4	13.2325	20.0112	0.0178005	0.550124	293.15	293.15	0	341.542	341.542	0.0775893	0.077564

610	68.23	13.1953	20.0008	0.0177514	0.543727	293.15	293.15	0	341.377	341.377	0.0775501	0.0775246

611	68.07	13.1287	20.0008	0.0176626	0.542365	293.15	293.15	0	341.219	341.219	0.0775119	0.0774867

612	67.9	13.0751	19.9966	0.0175915	0.538258	293.15	293.15	0	341.056	341.056	0.0774731	0.0774471

613	67.74	13.1068	19.9904	0.017635	0.532778	293.15	293.15	0	340.883	340.883	0.0774345	0.0774083

614	67.56	13.1783	19.9998	0.0177321	0.530487	293.15	293.15	0	340.712	340.712	0.0773943	0.0773683

615	67.4	13.1879	20.0008	0.0177459	0.525579	293.15	293.15	0	340.546	340.546	0.0773563	0.0773298

616	67.23	13.1824	20.0008	0.0177394	0.518314	293.15	293.15	0	340.38	340.38	0.0773179	0.0772903

617	67.06	13.2529	20.0008	0.0178352	0.515968	293.15	293.15	0	340.225	340.225	0.0772789	0.0772514

618	66.9	13.2672	20.0008	0.0178553	0.514055	293.15	293.15	0	340.055	340.055	0.0772396	0.0772122

619	66.73	13.2336	20.0008	0.017811	0.51186	293.15	293.15	0	339.879	339.879	0.0772003	0.0771728

620	66.56	13.2415	19.9946	0.0178226	0.508185	293.15	293.15	0	339.718	339.718	0.0771606	0.0771332

621	66.39	13.1933	20.0008	0.0177586	0.503995	293.15	293.15	0	339.558	339.558	0.0771221	0.0770949

622	66.23	13.0838	20.0008	0.017612	0.499255	293.15	293.15	0	339.385	339.385	0.0770832	0.0770561

623	66.06	12.983	20.0008	0.0174773	0.494823	293.15	293.15	0	339.217	339.217	0.0770448	0.0770162

624	65.89	12.9302	20.0008	0.0174071	0.489603	293.15	293.15	0	339.047	339.047	0.0770053	0.0769771

625	65.72	12.9434	20.0008	0.0174258	0.485865	293.15	293.15	0	338.891	338.891	0.076966	0.0769382

626	65.55	13.0142	20.0008	0.017522	0.482796	293.15	293.15	0	338.725	338.725	0.0769274	0.076899

627	65.38	13.1214	20.0008	0.0176672	0.480253	293.15	293.15	0	338.544	338.544	0.0768887	0.0768596

628	65.22	13.1708	20.0008	0.0177345	0.477736	293.15	293.15	0	338.388	338.388	0.07685	0.0768214

629	65.05	13.1579	20.0008	0.0177181	0.472072	293.15	293.15	0	338.224	338.224	0.0768106	0.0767822

630	64.88	13.1999	20.0008	0.0177755	0.469616	293.15	293.15	0	338.05	338.05	0.0767717	0.0767427

631	64.72	13.208	19.9956	0.0177873	0.466445	293.15	293.15	0	337.887	337.887	0.076733	0.0767037

632	64.55	13.2216	19.9904	0.0178067	0.459611	293.15	293.15	0	337.713	337.713	0.0766944	0.0766645

633	64.38	13.2835	19.9904	0.0178909	0.458033	293.15	293.15	0	337.558	337.558	0.0766549	0.0766247

634	64.21	13.3699	19.9998	0.0180081	0.456491	293.15	293.15	0	337.392	337.392	0.0766156	0.0765853

635	64.04	13.416	20.0008	0.0180712	0.452151	293.15	293.15	0	337.219	337.219	0.0765764	0.0765458

636	63.88	13.4654	20.0008	0.0181387	0.447302	293.15	293.15	0	337.048	337.048	0.0765384	0.0765077

637	63.71	13.4408	20.0008	0.0181064	0.441198	293.15	293.15	0	336.882	336.882	0.0764998	0.0764685

638	63.54	13.4616	20.0008	0.0181353	0.438584	293.15	293.15	0	336.711	336.711	0.0764601	0.0764295

639	63.38	13.4261	20.0008	0.0180885	0.435182	293.15	293.15	0	336.552	336.552	0.0764213	0.0763905

640	63.21	13.3764	20.0008	0.0180223	0.430787	293.15	293.15	0	336.379	336.379	0.0763824	0.0763513

641	63.04	13.4271	20.0008	0.0180917	0.427623	293.15	293.15	0	336.228	336.228	0.0763432	0.0763119

642	62.87	13.5166	20.0008	0.0182132	0.424231	293.15	293.15	0	336.049	336.049	0.0763036	0.0762718

643	62.7	13.5795	20.0008	0.0182989	0.41957	293.15	293.15	0	335.884	335.884	0.0762652	0.076233

644	62.54	13.5501	20.0008	0.0182602	0.415262	293.15	293.15	0	335.717	335.717	0.076227	0.0761941

645	62.37	13.4646	20.0008	0.0181458	0.412927	293.15	293.15	0	335.555	335.555	0.0761873	0.0761549

646	62.2	13.3944	19.9998	0.0180521	0.407355	293.15	293.15	0	335.389	335.389	0.0761481	0.0761159

647	62.03	13.3696	19.9904	0.0180196	0.406971	293.15	293.15	0	335.209	335.209	0.0761078	0.0760755

648	61.86	13.3477	19.9966	0.017991	0.401813	293.15	293.15	0	335.051	335.051	0.0760702	0.0760366

649	61.7	13.3098	20.0112	0.0179408	0.401153	293.15	293.15	0	334.887	334.887	0.0760306	0.0759977

650	61.53	13.305	20.0008	0.0179353	0.395455	293.15	293.15	0	334.714	334.714	0.0759916	0.0759594

651	61.37	13.2734	20.0008	0.0178935	0.392806	293.15	293.15	0	334.542	334.542	0.0759526	0.0759203

652	61.2	13.2327	20.0008	0.0178396	0.389006	293.15	293.15	0	334.377	334.377	0.0759138	0.0758812

653	61.03	13.1839	19.9966	0.0177747	0.385253	293.15	293.15	0	334.22	334.22	0.0758754	0.0758424

654	60.87	13.1417	19.9946	0.0177187	0.380914	293.15	293.15	0	334.04	334.04	0.0758365	0.0758036

655	60.7	13.1803	20.0008	0.0177717	0.376084	293.15	293.15	0	333.891	333.891	0.0757974	0.0757644

656	60.53	13.3118	20.0008	0.0179499	0.372475	293.15	293.15	0	333.718	333.718	0.0757586	0.0757245

657	60.36	13.434	20.0008	0.0181156	0.370691	293.15	293.15	0	333.548	333.548	0.075719	0.0756857

658	60.2	13.4606	20.0008	0.0181523	0.368037	293.15	293.15	0	333.389	333.389	0.0756801	0.0756461

659	60.03	13.4757	20.0008	0.0181737	0.362863	293.15	293.15	0	333.223	333.223	0.0756403	0.0756071

660	59.86	13.499	20.0008	0.018206	0.359262	293.15	293.15	0	333.055	333.055	0.0756016	0.0755677

661	59.69	13.5224	20.0008	0.0182386	0.354335	293.15	293.15	0	332.893	332.893	0.0755626	0.0755281

662	59.53	13.4972	20.0008	0.0182055	0.352202	293.15	293.15	0	332.728	332.728	0.0755236	0.0754899

663	59.36	13.4917	20.0008	0.0181989	0.34767	293.15	293.15	0	332.547	332.547	0.0754854	0.0754506

664	59.19	13.493	20.0008	0.0182016	0.34303	293.15	293.15	0	332.39	332.39	0.075446	0.0754113

665	59.02	13.4721	20.0008	0.0181743	0.34083	293.15	293.15	0	332.226	332.226	0.0754067	0.0753714

666	58.85	13.4691	20.0008	0.0181713	0.340026	293.15	293.15	0	332.053	332.053	0.0753671	0.0753319

667	58.68	13.4856	19.9904	0.0181944	0.337377	293.15	293.15	0	331.879	331.879	0.0753275	0.0752918

668	58.51	13.4769	19.9904	0.0181836	0.331052	293.15	293.15	0	331.714	331.714	0.0752884	0.0752527

669	58.35	13.4696	19.9998	0.0181746	0.327666	293.15	293.15	0	331.543	331.543	0.0752496	0.0752139

670	58.18	13.457	19.9946	0.0181585	0.324212	293.15	293.15	0	331.386	331.386	0.075211	0.0751751

671	58.01	13.4319	20.0008	0.0181256	0.321447	293.15	293.15	0	331.219	331.219	0.0751717	0.0751355

672	57.85	13.3917	20.0008	0.0180723	0.314197	293.15	293.15	0	331.05	331.05	0.0751333	0.075097

673	57.69	13.3656	20.0008	0.018038	0.311354	293.15	293.15	0	330.883	330.883	0.0750948	0.0750584

674	57.52	13.3596	20.0008	0.0180309	0.307589	293.15	293.15	0	330.704	330.704	0.0750559	0.0750193

675	57.35	13.3726	20.0008	0.0180493	0.305975	293.15	293.15	0	330.552	330.552	0.0750155	0.0749793

676	57.18	13.3897	20.0029	0.0180733	0.301774	293.15	293.15	0	330.379	330.379	0.074976	0.0749396

677	57.01	13.375	20.0112	0.0180544	0.296982	293.15	293.15	0	330.23	330.23	0.0749376	0.0749007

678	56.85	13.441	20.0112	0.0181443	0.287723	293.15	293.15	0	330.05	330.05	0.0749001	0.0748619

679	56.71	17.1568	19.9998	0.0231613	0.214936	293.15	293.15	0	329.883	329.883	0.0748928	0.0748293

680	56.64	29.2152	20.0019	0.0394407	0.110577	293.15	293.15	0	329.713	329.713	0.0749074	0.0748141

681	56.54	41.1711	20.006	0.0555831	0.0537706	293.15	293.15	0	329.555	329.555	0.0748928	0.0747904

682	56.37	50.7679	20.0008	0.0685427	0.0145032	293.15	293.15	0	329.39	329.39	0.0748623	0.0747512

683	56.18	58.8482	20.0008	0.0794568	-0.0136331	293.15	293.15	0	329.219	329.219	0.0748245	0.0747053

684	55.99	66.0477	20.0008	0.0891829	-0.043435	293.15	293.15	0	329.044	329.044	0.0747867	0.0746598

685	55.81	72.2753	20.0008	0.097597	-0.0764217	293.15	293.15	0	328.888	328.888	0.0747516	0.0746183

686	55.64	77.4517	20.0008	0.104592	-0.1158	293.15	293.15	0	328.717	328.717	0.0747162	0.0745798

687	55.49	81.4234	19.9966	0.109961	-0.15748	293.15	293.15	0	328.542	328.542	0.0746832	0.0745432

688	55.34	84.5753	19.9904	0.114223	-0.197011	293.15	293.15	0	328.379	328.379	0.0746497	0.0745078

689	55.19	87.0459	19.9987	0.117565	-0.239405	293.15	293.15	0	328.221	328.221	0.0746173	0.0744731

690	55.05	88.9367	20.0008	0.120123	-0.285554	293.15	293.15	0	328.048	328.048	0.0745846	0.07444

691	54.91	90.3664	20.0008	0.12206	-0.333323	293.15	293.15	0	327.884	327.884	0.0745537	0.0744074

692	54.77	91.4007	20.0008	0.123462	-0.382128	293.15	293.15	0	327.714	327.714	0.0745223	0.0743756

693	54.64	92.1449	19.9987	0.124472	-0.428237	293.15	293.15	0	327.563	327.563	0.0744909	0.0743445

694	54.51	92.6025	19.9904	0.125095	-0.485921	293.15	293.15	0	327.39	327.39	0.0744605	0.0743135

695	54.38	92.6808	19.9925	0.125206	-0.540042	293.15	293.15	0	327.221	327.221	0.074429	0.074283

696	54.24	92.503	20.0008	0.124971	-0.594752	293.15	293.15	0	327.053	327.053	0.0743966	0.0742513

697	54.11	92.1257	20.0008	0.124466	-0.653184	293.15	293.15	0	326.879	326.879	0.0743644	0.0742197

698	53.97	91.5602	19.9998	0.123707	-0.706086	293.15	293.15	0	326.721	326.721	0.0743314	0.0741881

699	53.84	90.7595	19.9914	0.122631	-0.759822	293.15	293.15	0	326.559	326.559	0.0742975	0.0741559

700	53.7	89.7957	20.0008	0.121333	-0.817042	293.15	293.15	0	326.384	326.384	0.0742635	0.0741233

701	53.56	88.6784	19.9998	0.119829	-0.870713	293.15	293.15	0	326.212	326.212	0.0742285	0.0740904

702	53.41	87.37	19.9904	0.118066	-0.926485	293.15	293.15	0	326.046	326.046	0.0741919	0.0740555

703	53.26	85.9032	19.9904	0.116089	-0.973139	293.15	293.15	0	325.891	325.891	0.0741544	0.07402

704	53.1	84.32	19.9956	0.113955	-1.02336	293.15	293.15	0	325.718	325.718	0.0741159	0.073984

705	52.95	82.5186	20.0008	0.111526	-1.06799	293.15	293.15	0	325.554	325.554	0.0740755	0.073947

706	52.79	80.4618	20.0008	0.108751	-1.11548	293.15	293.15	0	325.381	325.381	0.0740341	0.0739091

707	52.61	78.1862	20.0008	0.105681	-1.15319	293.15	293.15	0	325.224	325.224	0.0739903	0.0738684

708	52.43	75.7561	20.0008	0.102402	-1.18868	293.15	293.15	0	325.053	325.053	0.0739448	0.0738264

709	52.25	73.1941	20.0008	0.0989445	-1.21796	293.15	293.15	0	324.886	324.886	0.0738978	0.0737835

710	52.06	70.3497	20.0008	0.0951051	-1.24618	293.15	293.15	0	324.714	324.714	0.0738478	0.0737379

711	51.85	67.0639	20.0008	0.0906686	-1.26082	293.15	293.15	0	324.549	324.549	0.0737947	0.0736899

712	51.64	63.2703	20.0008	0.0855453	-1.26478	293.15	293.15	0	324.388	324.388	0.0737375	0.0736391

713	51.41	58.9806	20.0008	0.079751	-1.26219	293.15	293.15	0	324.229	324.229	0.073677	0.0735853

714	51.16	54.3786	20.0008	0.0735339	-1.24621	293.15	293.15	0	324.055	324.055	0.0736135	0.0735278

715	50.9	49.7938	20.0008	0.0673393	-1.22777	293.15	293.15	0	323.886	323.886	0.0735477	0.0734672

716	50.64	45.3164	20.0008	0.0612892	-1.19434	293.15	293.15	0	323.719	323.719	0.0734793	0.0734042

717	50.37	41.2276	20.0008	0.0557637	-1.15434	293.15	293.15	0	323.545	323.545	0.0734114	0.0733414

718	50.09	37.6879	19.9925	0.0509803	-1.11517	293.15	293.15	0	323.385	323.385	0.0733442	0.0732767

719	49.82	34.555	19.9904	0.0467463	-1.07014	293.15	293.15	0	323.215	323.215	0.0732758	0.0732118

720	49.54	31.9036	19.9977	0.0431631	-1.01745	293.15	293.15	0	323.048	323.048	0.0732083	0.0731475

721	49.26	29.5695	20.0008	0.0400086	-0.962777	293.15	293.15	0	322.884	322.884	0.0731421	0.0730818

722	48.99	27.6209	20.0008	0.0373751	-0.898193	293.15	293.15	0	322.712	322.712	0.0730756	0.0730172

723	48.72	26.0146	20.0008	0.0352046	-0.842996	293.15	293.15	0	322.555	322.555	0.0730105	0.0729528

724	48.44	24.7807	20.0008	0.0335375	-0.766256	293.15	293.15	0	322.374	322.374	0.0729464	0.0728891

725	48.18	23.8284	20.0008	0.0322513	-0.70354	293.15	293.15	0	322.226	322.226	0.0728837	0.072827

726	47.92	23.0532	19.9966	0.0312045	-0.629459	293.15	293.15	0	322.052	322.052	0.072822	0.0727652

727	47.66	22.4501	19.9904	0.0303906	-0.552703	293.15	293.15	0	321.881	321.881	0.0727615	0.0727049

728	47.41	21.9179	19.9998	0.0296725	-0.480482	293.15	293.15	0	321.713	321.713	0.0727012	0.0726449

729	47.16	21.4005	20.0039	0.0289741	-0.400125	293.15	293.15	0	321.553	321.553	0.0726416	0.0725862

730	46.91	20.9767	20.0112	0.0284026	-0.31178	293.15	293.15	0	321.376	321.376	0.0725836	0.0725283

731	46.67	20.6294	20.0029	0.0279344	-0.227807	293.15	293.15	0	321.212	321.212	0.0725266	0.0724712

732	46.43	20.2965	20.0008	0.0274856	-0.144649	293.15	293.15	0	321.052	321.052	0.0724691	0.072414

733	46.19	20.0117	20.0008	0.0271019	-0.0588781	293.15	293.15	0	320.883	320.883	0.0724137	0.0723588

734	45.96	19.7595	20.0008	0.0267622	0.031208	293.15	293.15	0	320.715	320.715	0.0723591	0.0723044

735	45.74	19.4714	20.0008	0.0263737	0.108135	293.15	293.15	0	320.561	320.561	0.0723077	0.0722534

736	45.59	18.984	20.0008	0.0257148	0.171335	293.15	293.15	0	320.387	320.387	0.0722713	0.0722181

737	45.51	17.7708	20.0008	0.024072	0.209367	293.15	293.15	0	320.215	320.215	0.0722459	0.0721973

738	45.45	15.8523	20.0008	0.0214737	0.229343	293.15	293.15	0	320.041	320.041	0.0722297	0.0721844

739	45.41	13.6376	20.0008	0.0184738	0.239729	293.15	293.15	0	319.894	319.894	0.0722164	0.0721753

740	45.38	11.5547	20.0008	0.0156524	0.238616	293.15	293.15	0	319.721	319.721	0.0722068	0.0721671

741	45.35	9.74687	20.0008	0.0132036	0.23132	293.15	293.15	0	319.548	319.548	0.0721976	0.0721596

742	45.31	8.35118	20.0008	0.011313	0.219144	293.15	293.15	0	319.384	319.384	0.0721882	0.0721517

743	45.26	7.3042	20.0008	0.00989488	0.206869	293.15	293.15	0	319.227	319.227	0.0721763	0.0721398

744	45.2	6.60026	20.0008	0.00894143	0.190563	293.15	293.15	0	319.055	319.055	0.0721626	0.072126

745	45.13	6.26479	20.0008	0.00848715	0.175743	293.15	293.15	0	318.889	318.889	0.0721462	0.0721091

746	45.04	6.24393	20.0008	0.00845911	0.160683	293.15	293.15	0	318.709	318.709	0.0721259	0.0720881

747	44.95	6.45928	20.0102	0.00875111	0.145023	293.15	293.15	0	318.544	318.544	0.0721056	0.0720668

748	44.85	6.81788	20.0019	0.00923722	0.129985	293.15	293.15	0	318.378	318.378	0.0720829	0.0720438

749	44.74	7.28793	20.0008	0.0098744	0.114276	293.15	293.15	0	318.222	318.222	0.0720581	0.0720173

750	44.62	7.86967	20.0008	0.010663	0.103738	293.15	293.15	0	318.053	318.053	0.0720296	0.0719877

751	44.48	8.46936	20.0008	0.011476	0.0946618	293.15	293.15	0	317.885	317.885	0.0719994	0.0719563

752	44.35	9.1039	20.0008	0.0123363	0.085967	293.15	293.15	0	317.712	317.712	0.0719673	0.0719241

753	44.2	9.73699	20.0008	0.0131948	0.0755316	293.15	293.15	0	317.564	317.564	0.0719356	0.0718902

754	44.05	10.3012	20.0008	0.01396	0.068033	293.15	293.15	0	317.397	317.397	0.0719011	0.0718554

755	43.9	10.7554	20.0008	0.0145761	0.0609702	293.15	293.15	0	317.219	317.219	0.0718663	0.0718201

756	43.75	11.1835	19.9935	0.0151571	0.0545374	293.15	293.15	0	317.05	317.05	0.0718302	0.0717833

757	43.59	11.5202	19.9977	0.0156142	0.0465404	293.15	293.15	0	316.881	316.881	0.0717936	0.0717465

758	43.43	11.8455	19.9987	0.0160558	0.0412958	293.15	293.15	0	316.708	316.708	0.0717564	0.0717095

759	43.27	12.1583	19.9904	0.0164806	0.0400819	293.15	293.15	0	316.56	316.56	0.0717177	0.0716697

760	43.1	12.4998	19.9914	0.0169444	0.0375357	293.15	293.15	0	316.393	316.393	0.071679	0.0716298

761	42.93	12.7535	20.0008	0.0172891	0.0332454	293.15	293.15	0	316.223	316.223	0.071641	0.0715917

762	42.77	12.8984	20.0008	0.0174866	0.0289979	293.15	293.15	0	316.048	316.048	0.0716024	0.0715527

763	42.6	13.045	20.0008	0.0176861	0.0293686	293.15	293.15	0	315.893	315.893	0.0715619	0.0715124

764	42.43	13.2229	19.9904	0.0179283	0.0276262	293.15	293.15	0	315.719	315.719	0.0715233	0.0714736

765	42.26	13.3397	20.0008	0.0180875	0.0226996	293.15	293.15	0	315.546	315.546	0.0714838	0.0714332

766	42.1	13.4217	20.0008	0.0181997	0.0229603	293.15	293.15	0	315.374	315.374	0.0714444	0.0713938

767	41.93	13.5044	19.9904	0.0183128	0.0213129	293.15	293.15	0	315.209	315.209	0.0714049	0.0713538

768	41.76	13.5947	20.0008	0.0184361	0.0210558	293.15	293.15	0	315.054	315.054	0.0713654	0.0713141

769	41.59	13.6511	20.0008	0.0185136	0.0183044	293.15	293.15	0	314.888	314.888	0.0713262	0.0712746

770	41.42	13.6678	20.0008	0.0185372	0.0148103	293.15	293.15	0	314.717	314.717	0.071286	0.0712353

771	41.26	13.6703	20.0008	0.0185415	0.0107617	293.15	293.15	0	314.551	314.551	0.0712479	0.0711964

772	41.09	13.7029	20.0008	0.0185867	0.00871549	293.15	293.15	0	314.386	314.386	0.0712084	0.0711567

773	40.93	13.7035	20.0008	0.0185884	0.00404154	293.15	293.15	0	314.225	314.225	0.071171	0.071119

774	40.77	13.6384	20.0008	0.0185011	-0.00207167	293.15	293.15	0	314.057	314.057	0.0711331	0.0710814

775	40.62	13.5087	20.0008	0.018326	-0.00989784	293.15	293.15	0	313.884	313.884	0.071096	0.0710446

776	40.46	13.328	19.9956	0.0180817	-0.0177524	293.15	293.15	0	313.714	313.714	0.0710596	0.0710081

777	40.31	13.1443	20.0008	0.0178332	-0.030172	293.15	293.15	0	313.547	313.547	0.0710232	0.0709726

778	40.16	13.0104	20.0008	0.0176524	-0.0424608	293.15	293.15	0	313.377	313.377	0.070988	0.0709371

779	40.01	12.9169	20.0008	0.0175263	-0.0562037	293.15	293.15	0	313.217	313.217	0.0709543	0.0709021

780	39.86	12.856	20.0008	0.0174444	-0.0718566	293.15	293.15	0	313.044	313.044	0.0709192	0.0708674

781	39.72	12.8001	20.0008	0.0173693	-0.0856605	293.15	293.15	0	312.894	312.894	0.0708842	0.0708334

782	39.58	12.7093	20.0008	0.0172469	-0.104225	293.15	293.15	0	312.723	312.723	0.0708505	0.0707999

783	39.44	12.5309	20.0008	0.0170055	-0.12743	293.15	293.15	0	312.548	312.548	0.0708179	0.0707669

784	39.3	12.3908	20.0008	0.0168162	-0.147459	293.15	293.15	0	312.384	312.384	0.0707845	0.0707335

785	39.16	12.2509	20.0008	0.0166269	-0.172126	293.15	293.15	0	312.22	312.22	0.0707531	0.0707017

786	39.03	12.0403	20.0008	0.0163418	-0.200223	293.15	293.15	0	312.055	312.055	0.0707208	0.0706704

787	38.9	11.9032	20.006	0.0161564	-0.231247	293.15	293.15	0	311.883	311.883	0.0706903	0.0706387

788	38.76	11.7706	20.0008	0.015977	-0.25817	293.15	293.15	0	311.718	311.718	0.0706581	0.0706073

789	38.63	11.6355	20.0008	0.0157942	-0.295576	293.15	293.15	0	311.545	311.545	0.0706278	0.0705769

790	38.51	11.5262	20.0008	0.0156465	-0.330623	293.15	293.15	0	311.388	311.388	0.0705983	0.0705472

791	38.39	11.4676	20.0008	0.0155675	-0.369347	293.15	293.15	0	311.222	311.222	0.0705694	0.0705185

792	38.26	11.3739	20.0008	0.0154409	-0.412595	293.15	293.15	0	311.053	311.053	0.0705391	0.070489

793	38.14	11.2406	20.0008	0.0152605	-0.457397	293.15	293.15	0	310.885	310.885	0.0705107	0.0704608

794	38.02	11.1041	20.0008	0.0150758	-0.507533	293.15	293.15	0	310.712	310.712	0.0704825	0.0704313

795	37.9	10.9871	20.0008	0.0149174	-0.552537	293.15	293.15	0	310.561	310.561	0.070454	0.0704038

796	37.78	10.8796	20.0008	0.0147721	-0.606446	293.15	293.15	0	310.391	310.391	0.0704269	0.0703762

797	37.67	10.7953	20.0008	0.0146581	-0.66488	293.15	293.15	0	310.218	310.218	0.0703997	0.0703487

798	37.56	10.6728	19.9956	0.0144923	-0.724281	293.15	293.15	0	310.05	310.05	0.0703733	0.0703224

799	37.44	10.5441	20.0008	0.0143179	-0.784073	293.15	293.15	0	309.888	309.888	0.070346	0.0702959

800	37.34	10.4587	20.0008	0.0142025	-0.851132	293.15	293.15	0	309.722	309.722	0.07032	0.0702703

801	37.23	10.3597	20.0008	0.0140685	-0.923561	293.15	293.15	0	309.542	309.542	0.070294	0.0702444

802	37.12	10.2586	20.0008	0.0139317	-0.990884	293.15	293.15	0	309.385	309.385	0.0702687	0.0702191

803	37.01	10.1279	20.0008	0.0137546	-1.06258	293.15	293.15	0	309.221	309.221	0.0702434	0.0701932

804	36.91	10.0187	19.9904	0.0136067	-1.1468	293.15	293.15	0	309.048	309.048	0.0702189	0.0701691

805	36.81	9.92337	20.0008	0.0134777	-1.22729	293.15	293.15	0	308.884	308.884	0.0701945	0.0701454

806	36.71	9.80111	20.0008	0.0133121	-1.3162	293.15	293.15	0	308.71	308.71	0.0701706	0.0701214

807	36.61	9.64498	20.0008	0.0131004	-1.40032	293.15	293.15	0	308.553	308.553	0.0701471	0.0700979

808	36.51	9.42879	20.0008	0.0128071	-1.49717	293.15	293.15	0	308.381	308.381	0.0701234	0.0700741

809	36.41	9.2805	20.0008	0.0126061	-1.59785	293.15	293.15	0	308.209	308.209	0.070101	0.0700516

810	36.31	9.19385	20.0008	0.0124888	-1.69197	293.15	293.15	0	308.052	308.052	0.0700783	0.0700285

811	36.22	9.1579	20.0008	0.0124403	-1.79468	293.15	293.15	0	307.886	307.886	0.0700562	0.0700067

812	36.13	9.12834	20.006	0.0124005	-1.90585	293.15	293.15	0	307.717	307.717	0.0700335	0.0699847

813	36.03	9.10827	20.0008	0.0123736	-2.01852	293.15	293.15	0	307.549	307.549	0.070012	0.0699627

814	35.94	9.04437	20.0008	0.0122871	-2.13813	293.15	293.15	0	307.376	307.376	0.0699908	0.0699404

815	35.85	8.9549	20.0039	0.0121659	-2.25503	293.15	293.15	0	307.212	307.212	0.0699687	0.0699187

816	35.76	8.90873	20.0091	0.0121035	-2.36868	293.15	293.15	0	307.061	307.061	0.0699483	0.0698984

817	35.67	8.8256	20.0008	0.0119909	-2.50744	293.15	293.15	0	306.882	306.882	0.069928	0.0698775

818	35.59	8.68127	20.006	0.0117951	-2.63921	293.15	293.15	0	306.715	306.715	0.0699075	0.0698578

819	35.51	8.58366	20.0008	0.0116628	-2.77884	293.15	293.15	0	306.545	306.545	0.0698873	0.0698376

820	35.43	8.4729	20.0008	0.0115126	-2.91841	293.15	293.15	0	306.379	306.379	0.069868	0.0698186

821	35.34	8.33102	20.0008	0.0113201	-3.05607	293.15	293.15	0	306.224	306.224	0.0698489	0.0697992

822	35.26	8.21157	20.0008	0.011158	-3.20365	293.15	293.15	0	306.058	306.058	0.0698295	0.0697801

823	35.19	8.09949	20.0008	0.011006	-3.36892	293.15	293.15	0	305.878	305.878	0.0698104	0.0697619

824	35.11	8.06405	20.0008	0.0109581	-3.51851	293.15	293.15	0	305.721	305.721	0.0697923	0.0697431

825	35.03	8.10365	19.9904	0.0110122	-3.67947	293.15	293.15	0	305.557	305.557	0.0697738	0.0697253

826	34.95	8.10543	20.0008	0.0110148	-3.85407	293.15	293.15	0	305.383	305.383	0.0697562	0.0697066

827	34.88	8.07106	20.0008	0.0109684	-4.02149	293.15	293.15	0	305.22	305.22	0.0697377	0.0696888

828	34.8	7.97819	20.0008	0.0108424	-4.20544	293.15	293.15	0	305.045	305.045	0.06972	0.069671

829	34.73	7.82511	19.9966	0.0106346	-4.3757	293.15	293.15	0	304.89	304.89	0.0697028	0.0696539

830	34.65	7.68204	19.9904	0.0104404	-4.56925	293.15	293.15	0	304.716	304.716	0.0696854	0.0696357

831	34.59	7.577	19.9998	0.0102979	-4.75524	293.15	293.15	0	304.552	304.552	0.0696677	0.0696203

832	34.51	7.48948	20.0008	0.0101792	-4.9456	293.15	293.15	0	304.39	304.39	0.0696515	0.0696033

833	34.44	7.4498	20.0008	0.0101254	-5.14898	293.15	293.15	0	304.223	304.223	0.0696354	0.0695866

834	34.38	7.43769	20.0008	0.0101092	-5.35741	293.15	293.15	0	304.053	304.053	0.0696191	0.0695708

835	34.31	7.38077	19.9977	0.010032	-5.56893	293.15	293.15	0	303.885	303.885	0.0696036	0.0695556

836	34.24	7.31891	19.9904	0.00994816	-5.78789	293.15	293.15	0	303.715	303.715	0.0695878	0.0695391

837	34.18	7.26201	19.9998	0.009871	-5.99928	293.15	293.15	0	303.556	303.556	0.0695725	0.0695243

838	34.11	7.1438	20.0091	0.00971052	-6.23376	293.15	293.15	0	303.383	303.383	0.069557	0.0695086

839	34.05	7.03019	20.0008	0.00955628	-25.145	293.15	293.15	0	242.592	242.592	0.0695425	0.0694936
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RT54-0.2 GNP.txt
# Name: RT54-0.2 GNP 2

# Date: Tue May 21 10:46:37 2024

# Weight: 10 mg

Time(s)	Temperature(°C)	Heat flow(mW)	Gas 1(sccm/min)	DSC_RAW(µV)	POWER(%)	TEMP_CJR_FURNACE(K)	TEMP_CJR_SAMPLE(K)	TEMP_FURNACE(K)	TEMP_NOM_FURNACE(K)	TEMP_NOM_SAMPLE(K)	VOLTAGE_REFERENCE(V)	VOLTAGE_SAMPLE(V)

0	29.85	-0.01805	20.0008	-2.45672e-05	0.0900143	293.15	293.15	0	303.276	303.276	0.0685537	0.068498

1	29.87	-0.0347912	20.0008	-4.73528e-05	0.15178	293.15	293.15	0	303.449	303.449	0.0685588	0.0685037

2	29.96	-0.397176	19.9946	-0.000540565	0.193927	293.15	293.15	0	303.606	303.606	0.0685766	0.0685238

3	30.08	-1.38421	19.9956	-0.00188387	0.225822	293.15	293.15	0	303.771	303.771	0.0686029	0.0685538

4	30.24	-2.85764	20.0008	-0.00388897	0.251547	293.15	293.15	0	303.943	303.943	0.0686368	0.0685911

5	30.41	-4.54361	19.9956	-0.00618308	0.265521	293.15	293.15	0	304.108	304.108	0.0686757	0.0686324

6	30.6	-6.25231	19.9956	-0.00850787	0.276214	293.15	293.15	0	304.281	304.281	0.068717	0.0686753

7	30.78	-7.82021	20.0008	-0.0106408	0.284448	293.15	293.15	0	304.436	304.436	0.0687599	0.0687196

8	30.98	-9.13948	20.0008	-0.0124351	0.291677	293.15	293.15	0	304.602	304.602	0.0688038	0.068766

9	31.17	-10.1656	20.0008	-0.0138305	0.295803	293.15	293.15	0	304.775	304.775	0.0688489	0.0688117

10	31.36	-10.9688	20.0008	-0.0149224	0.297981	293.15	293.15	0	304.947	304.947	0.0688942	0.0688575

11	31.55	-11.5529	20.0008	-0.0157162	0.300028	293.15	293.15	0	305.113	305.113	0.0689381	0.0689017

12	31.74	-11.9739	20.0008	-0.0162879	0.303028	293.15	293.15	0	305.278	305.278	0.0689832	0.0689465

13	31.93	-12.297	20.0008	-0.0167264	0.30353	293.15	293.15	0	305.434	305.434	0.0690279	0.0689922

14	32.11	-12.4889	20.0008	-0.0169864	0.304053	293.15	293.15	0	305.603	305.603	0.0690701	0.069035

15	32.3	-12.5548	20.0008	-0.0170751	0.305415	293.15	293.15	0	305.779	305.779	0.0691141	0.0690792

16	32.48	-12.5774	20.0008	-0.017105	0.306141	293.15	293.15	0	305.949	305.949	0.0691567	0.0691211

17	32.66	-12.6277	20.0008	-0.0171724	0.307381	293.15	293.15	0	306.116	306.116	0.0691987	0.0691642

18	32.83	-12.6205	20.0008	-0.0171617	0.307432	293.15	293.15	0	306.271	306.271	0.06924	0.0692051

19	33.01	-12.5527	20.0008	-0.0170686	0.312096	293.15	293.15	0	306.437	306.437	0.0692819	0.0692463

20	33.18	-12.4625	20.0008	-0.016945	0.313191	293.15	293.15	0	306.605	306.605	0.0693232	0.0692879

21	33.35	-12.3666	19.9935	-0.0168138	0.315575	293.15	293.15	0	306.775	306.775	0.0693631	0.0693287

22	33.53	-12.2781	19.9977	-0.0166926	0.317082	293.15	293.15	0	306.948	306.948	0.0694046	0.0693699

23	33.7	-12.2293	20.0008	-0.0166253	0.320096	293.15	293.15	0	307.112	307.112	0.0694452	0.0694104

24	33.87	-12.1345	20.0008	-0.0164956	0.322398	293.15	293.15	0	307.27	307.27	0.0694855	0.0694502

25	34.04	-12.048	20.0008	-0.0163771	0.326255	293.15	293.15	0	307.433	307.433	0.0695255	0.0694904

26	34.21	-11.9666	20.0008	-0.0162657	0.325454	293.15	293.15	0	307.607	307.607	0.0695656	0.0695302

27	34.37	-11.898	20.0008	-0.0161716	0.331809	293.15	293.15	0	307.779	307.779	0.069605	0.0695698

28	34.54	-11.8895	19.9956	-0.0161592	0.334433	293.15	293.15	0	307.943	307.943	0.0696453	0.0696104

29	34.71	-11.901	20.0008	-0.016174	0.336539	293.15	293.15	0	308.1	308.1	0.0696848	0.0696501

30	34.88	-11.8717	19.9956	-0.0161334	0.339717	293.15	293.15	0	308.273	308.273	0.0697233	0.0696885

31	35.05	-11.8221	19.9956	-0.0160652	0.341683	293.15	293.15	0	308.437	308.437	0.0697629	0.0697288

32	35.22	-11.8018	20.0008	-0.0160367	0.346484	293.15	293.15	0	308.611	308.611	0.0698035	0.0697691

33	35.38	-11.8005	20.0008	-0.0160342	0.347838	293.15	293.15	0	308.775	308.775	0.0698428	0.0698079

34	35.55	-11.781	20.0008	-0.0160068	0.35028	293.15	293.15	0	308.947	308.947	0.0698822	0.0698476

35	35.72	-11.7312	20.0008	-0.0159383	0.354566	293.15	293.15	0	309.103	309.103	0.0699213	0.0698877

36	35.89	-11.717	19.9966	-0.0159183	0.357734	293.15	293.15	0	309.269	309.269	0.0699611	0.0699277

37	36.05	-11.6835	19.9946	-0.015872	0.362049	293.15	293.15	0	309.442	309.442	0.0700003	0.0699668

38	36.22	-11.6676	20.0008	-0.0158495	0.366968	293.15	293.15	0	309.613	309.613	0.0700395	0.0700069

39	36.39	-11.7386	20.0008	-0.0159451	0.371917	293.15	293.15	0	309.779	309.779	0.0700784	0.0700458

40	36.56	-11.835	20.0008	-0.0160752	0.374192	293.15	293.15	0	309.945	309.945	0.0701189	0.0700868

41	36.73	-11.9133	20.0008	-0.0161808	0.374379	293.15	293.15	0	310.105	310.105	0.0701587	0.0701262

42	36.9	-11.9468	20.0008	-0.0162254	0.376597	293.15	293.15	0	310.273	310.273	0.0701988	0.0701661

43	37.06	-11.9005	19.9925	-0.0161618	0.381839	293.15	293.15	0	310.446	310.446	0.070237	0.0702054

44	37.23	-11.8692	19.9904	-0.0161184	0.386216	293.15	293.15	0	310.616	310.616	0.0702759	0.0702449

45	37.4	-11.873	19.9904	-0.0161227	0.387044	293.15	293.15	0	310.767	310.767	0.0703161	0.0702848

46	37.56	-11.8568	19.9977	-0.0160999	0.390829	293.15	293.15	0	310.94	310.94	0.0703552	0.0703238

47	37.73	-11.8041	20.0008	-0.0160275	0.393474	293.15	293.15	0	311.104	311.104	0.0703942	0.0703629

48	37.9	-11.7663	20.0008	-0.0159755	0.397674	293.15	293.15	0	311.271	311.271	0.0704346	0.0704033

49	38.07	-11.786	20.0008	-0.0160013	0.40098	293.15	293.15	0	311.441	311.441	0.0704739	0.0704428

50	38.23	-11.7869	20.0008	-0.0160018	0.406744	293.15	293.15	0	311.615	311.615	0.0705121	0.0704816

51	38.4	-11.7809	20.0008	-0.0159928	0.411607	293.15	293.15	0	311.764	311.764	0.0705508	0.0705208

52	38.57	-11.7701	20.0008	-0.0159774	0.410954	293.15	293.15	0	311.935	311.935	0.0705914	0.0705611

53	38.73	-11.8036	19.9998	-0.016022	0.415522	293.15	293.15	0	312.108	312.108	0.0706306	0.0706004

54	38.9	-11.8052	19.9904	-0.0160233	0.417533	293.15	293.15	0	312.274	312.274	0.0706701	0.0706398

55	39.07	-11.815	19.9966	-0.0160358	0.422812	293.15	293.15	0	312.446	312.446	0.0707091	0.07068

56	39.24	-11.8099	20.0008	-0.0160281	0.425954	293.15	293.15	0	312.619	312.619	0.0707487	0.070719

57	39.4	-11.7924	20.0008	-0.0160035	0.428047	293.15	293.15	0	312.768	312.768	0.0707878	0.0707578

58	39.57	-11.7981	20.0008	-0.0160104	0.42844	293.15	293.15	0	312.94	312.94	0.0708277	0.0707984

59	39.74	-11.8814	20.0008	-0.0161226	0.432389	293.15	293.15	0	313.104	313.104	0.0708662	0.0708376

60	39.91	-11.9602	20.0008	-0.0162287	0.43777	293.15	293.15	0	313.277	313.277	0.0709065	0.0708779

61	40.07	-12.0004	20.0008	-0.0162824	0.442206	293.15	293.15	0	313.451	313.451	0.070945	0.0709164

62	40.24	-12.0102	19.9966	-0.0162949	0.444452	293.15	293.15	0	313.614	313.614	0.0709841	0.0709559

63	40.41	-12.0037	19.9998	-0.0162852	0.447464	293.15	293.15	0	313.771	313.771	0.0710238	0.0709956

64	40.57	-11.9963	19.9966	-0.0162744	0.45242	293.15	293.15	0	313.944	313.944	0.0710632	0.0710346

65	40.74	-11.9418	19.9904	-0.0161996	0.453879	293.15	293.15	0	314.108	314.108	0.0711028	0.071074

66	40.9	-11.9284	19.9904	-0.0161807	0.459271	293.15	293.15	0	314.272	314.272	0.0711409	0.0711129

67	41.08	-11.8455	19.9904	-0.0160674	0.459872	293.15	293.15	0	314.438	314.438	0.0711818	0.0711534

68	41.24	-11.8046	19.9987	-0.016011	0.466519	293.15	293.15	0	314.607	314.607	0.0712201	0.0711922

69	41.41	-11.8669	20.0091	-0.0160947	0.470158	293.15	293.15	0	314.775	314.775	0.071259	0.0712319

70	41.58	-11.9183	20.0081	-0.0161636	0.47061	293.15	293.15	0	314.948	314.948	0.0712989	0.0712714

71	41.74	-11.9527	20.0008	-0.0162095	0.475031	293.15	293.15	0	315.099	315.099	0.0713373	0.0713106

72	41.91	-11.9314	20.0008	-0.0161798	0.479942	293.15	293.15	0	315.27	315.27	0.0713772	0.0713498

73	42.08	-11.8932	20.0008	-0.0161271	0.484174	293.15	293.15	0	315.442	315.442	0.0714162	0.0713899

74	42.25	-11.9136	20.0008	-0.016154	0.486918	293.15	293.15	0	315.61	315.61	0.0714558	0.0714292

75	42.42	-11.994	20.0008	-0.0162621	0.492169	293.15	293.15	0	315.78	315.78	0.0714952	0.0714691

76	42.59	-12.0348	19.9987	-0.0163166	0.492719	293.15	293.15	0	315.945	315.945	0.0715349	0.0715092

77	42.75	-12.019	19.9904	-0.0162944	0.493029	293.15	293.15	0	316.101	316.101	0.0715751	0.0715487

78	42.91	-11.9931	19.9956	-0.0162584	0.501553	293.15	293.15	0	316.266	316.266	0.0716124	0.0715864

79	43.08	-11.9746	19.9904	-0.0162325	0.501463	293.15	293.15	0	316.438	316.438	0.0716522	0.0716266

80	43.25	-12.0014	19.9904	-0.0162681	0.508922	293.15	293.15	0	316.611	316.611	0.0716913	0.0716656

81	43.41	-12.035	19.9914	-0.0163128	0.511138	293.15	293.15	0	316.776	316.776	0.0717302	0.0717044

82	43.58	-12.0844	20.0008	-0.0163789	0.512574	293.15	293.15	0	316.939	316.939	0.07177	0.0717448

83	43.75	-12.131	20.0008	-0.0164412	0.514251	293.15	293.15	0	317.105	317.105	0.0718097	0.0717838

84	43.92	-12.1465	20.0008	-0.0164614	0.521764	293.15	293.15	0	317.269	317.269	0.0718485	0.0718231

85	44.09	-12.0992	19.9904	-0.0163965	0.522419	293.15	293.15	0	317.442	317.442	0.0718883	0.0718634

86	44.25	-12.0624	19.9904	-0.0163457	0.527847	293.15	293.15	0	317.615	317.615	0.0719264	0.0719025

87	44.42	-12.0335	19.9904	-0.0163058	0.527072	293.15	293.15	0	317.78	317.78	0.0719668	0.0719425

88	44.59	-12.0678	19.9904	-0.0163514	0.53356	293.15	293.15	0	317.945	317.945	0.0720063	0.0719814

89	44.76	-12.1315	19.9946	-0.0164368	0.537393	293.15	293.15	0	318.108	318.108	0.0720448	0.0720208

90	44.93	-12.1968	20.0008	-0.0165245	0.539542	293.15	293.15	0	318.274	318.274	0.0720846	0.0720607

91	45.09	-12.2256	20.0008	-0.0165626	0.543568	293.15	293.15	0	318.447	318.447	0.0721241	0.0720998

92	45.25	-12.234	19.9966	-0.0165733	0.549401	293.15	293.15	0	318.618	318.618	0.0721628	0.0721382

93	45.42	-12.2083	19.9987	-0.0165376	0.552939	293.15	293.15	0	318.767	318.767	0.0722013	0.0721775

94	45.59	-12.1358	20.0008	-0.0164385	0.555319	293.15	293.15	0	318.941	318.941	0.072241	0.0722173

95	45.76	-12.0994	20.0008	-0.0163883	0.558666	293.15	293.15	0	319.105	319.105	0.0722799	0.0722566

96	45.92	-12.0732	20.0008	-0.0163521	0.565947	293.15	293.15	0	319.274	319.274	0.072318	0.0722953

97	46.09	-12.0977	20.0008	-0.0163844	0.56769	293.15	293.15	0	319.442	319.442	0.0723577	0.0723351

98	46.26	-12.1884	20.0008	-0.0165065	0.569166	293.15	293.15	0	319.612	319.612	0.0723973	0.0723746

99	46.43	-12.1954	20.0008	-0.0165151	0.573056	293.15	293.15	0	319.772	319.772	0.0724368	0.0724142

100	46.6	-12.118	20.0008	-0.0164094	0.577315	293.15	293.15	0	319.945	319.945	0.0724769	0.0724539

101	46.76	-12.0642	20.0008	-0.0163357	0.581587	293.15	293.15	0	320.104	320.104	0.0725153	0.0724927

102	46.92	-12.1089	19.9946	-0.0163954	0.58625	293.15	293.15	0	320.275	320.275	0.0725538	0.0725313

103	47.1	-12.1682	19.9966	-0.0164748	0.587445	293.15	293.15	0	320.44	320.44	0.0725932	0.0725717

104	47.26	-12.1467	20.0008	-0.0164449	0.593207	293.15	293.15	0	320.606	320.606	0.0726328	0.072611

105	47.43	-12.0815	20.0008	-0.0163559	0.59753	293.15	293.15	0	320.776	320.776	0.0726717	0.0726502

106	47.59	-12.0447	20.0008	-0.0163052	0.598955	293.15	293.15	0	320.943	320.943	0.0727109	0.0726889

107	47.76	-12.052	20.0008	-0.0163142	0.602641	293.15	293.15	0	321.097	321.097	0.0727501	0.0727288

108	47.93	-12.0728	20.0008	-0.0163416	0.604649	293.15	293.15	0	321.28	321.28	0.0727896	0.0727675

109	48.1	-12.1258	20.0008	-0.0164125	0.609596	293.15	293.15	0	321.443	321.443	0.0728289	0.0728076

110	48.27	-12.168	20.0008	-0.0164687	0.611206	293.15	293.15	0	321.608	321.608	0.0728685	0.0728478

111	48.43	-12.1743	20.0008	-0.0164765	0.616421	293.15	293.15	0	321.781	321.781	0.0729074	0.0728868

112	48.6	-12.2023	20.0008	-0.0165135	0.616755	293.15	293.15	0	321.945	321.945	0.0729471	0.0729261

113	48.77	-12.195	20.0008	-0.0165028	0.624233	293.15	293.15	0	322.102	322.102	0.0729857	0.0729646

114	48.93	-12.1683	19.9966	-0.0164659	0.628039	293.15	293.15	0	322.275	322.275	0.0730245	0.0730032

115	49.1	-12.1952	19.9946	-0.0165014	0.631424	293.15	293.15	0	322.447	322.447	0.0730641	0.0730437

116	49.27	-12.2526	19.9914	-0.0165782	0.637245	293.15	293.15	0	322.612	322.612	0.0731026	0.0730824

117	49.44	-12.2884	19.9904	-0.0166258	0.640274	293.15	293.15	0	322.769	322.769	0.0731421	0.0731222

118	49.61	-12.3033	19.9987	-0.0166451	0.644151	293.15	293.15	0	322.939	322.939	0.0731812	0.0731619

119	49.77	-12.3193	20.0008	-0.0166659	0.645839	293.15	293.15	0	323.106	323.106	0.0732198	0.0732005

120	49.94	-12.3351	20.0008	-0.0166864	0.650221	293.15	293.15	0	323.28	323.28	0.0732595	0.0732406

121	50.11	-12.298	20.0008	-0.0166354	0.654	293.15	293.15	0	323.443	323.443	0.0732989	0.0732799

122	50.28	-12.2741	19.9925	-0.0166022	0.657205	293.15	293.15	0	323.613	323.613	0.073338	0.0733195

123	50.44	-12.2982	19.9925	-0.016634	0.657679	293.15	293.15	0	323.764	323.764	0.0733776	0.0733583

124	50.61	-12.3166	19.9935	-0.016658	0.66482	293.15	293.15	0	323.941	323.941	0.0734165	0.0733974

125	50.77	-12.2868	19.9904	-0.0166169	0.66833	293.15	293.15	0	324.111	324.111	0.0734562	0.0734361

126	50.94	-12.2003	19.9925	-0.0164991	0.672953	293.15	293.15	0	324.284	324.284	0.0734944	0.0734756

127	51.11	-12.1823	20.0071	-0.0164738	0.674453	293.15	293.15	0	324.432	324.432	0.0735331	0.0735152

128	51.28	-12.1816	19.9987	-0.0164721	0.681345	293.15	293.15	0	324.597	324.597	0.0735723	0.0735544

129	51.44	-12.1981	19.9914	-0.0164936	0.687263	293.15	293.15	0	324.769	324.769	0.0736107	0.0735935

130	51.61	-12.2018	20.0008	-0.0164977	0.687201	293.15	293.15	0	324.942	324.942	0.0736511	0.0736334

131	51.78	-12.2264	20.0008	-0.0165301	0.688979	293.15	293.15	0	325.108	325.108	0.0736898	0.0736727

132	51.95	-12.2671	20.0008	-0.0165843	0.696232	293.15	293.15	0	325.279	325.279	0.0737294	0.0737123

133	52.11	-12.343	19.9956	-0.0166861	0.700451	293.15	293.15	0	325.437	325.437	0.0737682	0.0737513

134	52.28	-12.4042	19.9956	-0.0167679	0.703863	293.15	293.15	0	325.609	325.609	0.0738058	0.0737896

135	52.45	-12.4078	19.9904	-0.0167719	0.705533	293.15	293.15	0	325.773	325.773	0.0738458	0.0738294

136	52.61	-12.4585	19.9956	-0.0168397	0.709242	293.15	293.15	0	325.946	325.946	0.073885	0.0738688

137	52.79	-12.5381	20.0008	-0.0169464	0.712461	293.15	293.15	0	326.11	326.11	0.0739252	0.073909

138	52.95	-12.581	20.0008	-0.0170035	0.715899	293.15	293.15	0	326.276	326.276	0.0739639	0.0739478

139	53.11	-12.5763	20.0008	-0.0169962	0.719047	293.15	293.15	0	326.431	326.431	0.0740028	0.0739863

140	53.28	-12.5585	20.0008	-0.0169713	0.725314	293.15	293.15	0	326.603	326.603	0.0740418	0.0740259

141	53.45	-12.6131	19.9914	-0.0170444	0.731411	293.15	293.15	0	326.777	326.777	0.07408	0.0740648

142	53.62	-12.6655	19.9946	-0.0171142	0.733751	293.15	293.15	0	326.948	326.948	0.0741199	0.0741045

143	53.79	-12.6795	20.0008	-0.0171323	0.738031	293.15	293.15	0	327.115	327.115	0.0741591	0.0741442

144	53.95	-12.7317	19.9914	-0.017202	0.742876	293.15	293.15	0	327.269	327.269	0.0741974	0.0741828

145	54.12	-12.7364	19.9935	-0.0172074	0.746347	293.15	293.15	0	327.435	327.435	0.0742372	0.0742228

146	54.29	-12.763	20.0008	-0.0172424	0.748554	293.15	293.15	0	327.605	327.605	0.0742765	0.0742621

147	54.46	-12.7188	20.0008	-0.0171819	0.751014	293.15	293.15	0	327.773	327.773	0.0743157	0.0743014

148	54.63	-12.6859	20.0008	-0.0171366	0.75617	293.15	293.15	0	327.946	327.946	0.074355	0.074341

149	54.79	-12.7153	20.0008	-0.0171755	0.761034	293.15	293.15	0	328.115	328.115	0.0743934	0.0743796

150	54.96	-12.7627	20.0008	-0.0172385	0.761408	293.15	293.15	0	328.274	328.274	0.0744333	0.0744189

151	55.12	-12.7774	20.0008	-0.0172576	0.766033	293.15	293.15	0	328.44	328.44	0.0744719	0.0744579

152	55.29	-12.7729	20.0008	-0.0172505	0.771566	293.15	293.15	0	328.608	328.608	0.0745111	0.074497

153	55.46	-12.7798	20.0081	-0.0172591	0.776808	293.15	293.15	0	328.777	328.777	0.074549	0.0745358

154	55.62	-12.8218	20.0091	-0.0173149	0.783025	293.15	293.15	0	328.951	328.951	0.074588	0.0745749

155	55.79	-12.9016	20.0008	-0.0174218	0.787552	293.15	293.15	0	329.115	329.115	0.0746268	0.0746142

156	55.96	-13.0015	20.0008	-0.0175558	0.791642	293.15	293.15	0	329.273	329.273	0.074666	0.074654

157	56.16	-13.0123	20.0008	-0.0175693	0.762746	293.15	293.15	0	329.435	329.435	0.0747153	0.0747015

158	56.66	-13.7362	20.0008	-0.0185438	0.656881	293.15	293.15	0	329.608	329.608	0.074821	0.074819

159	56.75	-17.0511	20.0008	-0.0230183	0.681737	293.15	293.15	0	329.774	329.774	0.074842	0.07484

160	56.79	-17.1329	20.0008	-0.0231286	0.716643	293.15	293.15	0	329.946	329.946	0.0748585	0.0748491

161	56.87	-15.7531	20.0008	-0.0212654	0.743199	293.15	293.15	0	330.103	330.103	0.0748799	0.0748676

162	56.98	-14.2394	20.0008	-0.0192214	0.765297	293.15	293.15	0	330.276	330.276	0.074907	0.0748928

163	57.1	-13.1444	20.0008	-0.0177426	0.784783	293.15	293.15	0	330.448	330.448	0.0749366	0.0749222

164	57.24	-12.5354	20.0008	-0.0169198	0.798803	293.15	293.15	0	330.603	330.603	0.0749685	0.0749551

165	57.4	-12.4082	20.0008	-0.0167474	0.815612	293.15	293.15	0	330.769	330.769	0.0750031	0.0749913

166	57.56	-12.6548	19.9914	-0.0170794	0.828554	293.15	293.15	0	330.941	330.941	0.0750387	0.0750279

167	57.72	-13.038	19.9904	-0.0175957	0.838284	293.15	293.15	0	331.107	331.107	0.075076	0.0750659

168	57.88	-13.5733	19.9946	-0.0183171	0.850142	293.15	293.15	0	331.28	331.28	0.0751134	0.075105

169	58.05	-14.2716	20.0008	-0.0192586	0.860343	293.15	293.15	0	331.444	331.444	0.0751513	0.0751444

170	58.23	-15.1333	20.0008	-0.0204203	0.868563	293.15	293.15	0	331.607	331.607	0.0751909	0.0751853

171	58.4	-16.1282	19.9925	-0.0217616	0.878391	293.15	293.15	0	331.774	331.774	0.0752285	0.0752251

172	58.57	-17.2777	19.9987	-0.0233115	0.887536	293.15	293.15	0	331.944	331.944	0.0752669	0.0752655

173	58.74	-18.6109	20.0008	-0.025109	0.902644	293.15	293.15	0	332.112	332.112	0.0753036	0.0753051

174	58.91	-20.1778	20.0008	-0.0272215	0.913235	293.15	293.15	0	332.285	332.285	0.0753417	0.0753455

175	59.08	-21.9648	20.0008	-0.0296307	0.926501	293.15	293.15	0	332.433	332.433	0.0753777	0.0753848

176	59.25	-23.9999	20.0008	-0.0323745	0.942504	293.15	293.15	0	332.6	332.6	0.0754132	0.0754241

177	59.42	-26.4459	19.9935	-0.0356722	0.961704	293.15	293.15	0	332.77	332.77	0.0754489	0.0754642

178	59.59	-29.2918	19.9977	-0.0395089	0.981968	293.15	293.15	0	332.946	332.946	0.0754834	0.0755039

179	59.75	-32.4117	20.0008	-0.0437149	1.00391	293.15	293.15	0	333.116	333.116	0.0755176	0.0755424

180	59.92	-35.8517	19.9935	-0.048352	1.02274	293.15	293.15	0	333.282	333.282	0.0755523	0.0755827

181	60.09	-39.4688	19.9966	-0.0532276	1.04886	293.15	293.15	0	333.437	333.437	0.0755861	0.0756217

182	60.26	-43.2854	19.9998	-0.0583715	1.0707	293.15	293.15	0	333.602	333.602	0.0756205	0.0756622

183	60.44	-47.1697	19.9966	-0.0636064	1.09398	293.15	293.15	0	333.773	333.773	0.0756552	0.0757027

184	60.62	-51.0586	20.0008	-0.0688467	1.11495	293.15	293.15	0	333.947	333.947	0.0756918	0.0757445

185	60.8	-54.691	20.0008	-0.0737405	1.13433	293.15	293.15	0	334.111	334.111	0.0757298	0.0757872

186	60.98	-58.0841	20.0008	-0.078311	1.14579	293.15	293.15	0	334.267	334.267	0.0757702	0.0758307

187	61.17	-61.2395	20.0008	-0.0825606	1.16261	293.15	293.15	0	334.441	334.441	0.0758098	0.0758741

188	61.36	-64.0539	20.0008	-0.0863499	1.17291	293.15	293.15	0	334.605	334.605	0.0758514	0.0759187

189	61.55	-66.5131	20.0008	-0.0896598	1.18638	293.15	293.15	0	334.778	334.778	0.0758935	0.0759638

190	61.75	-68.5887	20.0008	-0.0924523	1.194	293.15	293.15	0	334.951	334.951	0.0759367	0.0760094

191	61.94	-70.3183	20.0008	-0.0947781	1.19801	293.15	293.15	0	335.116	335.116	0.0759801	0.0760551

192	62.14	-71.8026	20.0008	-0.096773	1.20069	293.15	293.15	0	335.271	335.271	0.0760251	0.0761002

193	62.33	-72.9385	19.9966	-0.0982982	1.2079	293.15	293.15	0	335.436	335.436	0.0760691	0.0761453

194	62.52	-73.7642	19.9998	-0.0994052	1.21104	293.15	293.15	0	335.608	335.608	0.0761127	0.0761899

195	62.71	-74.3168	20.0008	-0.100144	1.21243	293.15	293.15	0	335.774	335.774	0.0761569	0.0762344

196	62.9	-74.6192	20.0008	-0.100546	1.21229	293.15	293.15	0	335.947	335.947	0.0762013	0.0762789

197	63.09	-74.7277	20.0008	-0.100686	1.21263	293.15	293.15	0	336.1	336.1	0.0762456	0.0763231

198	63.27	-74.6047	20.0008	-0.100515	1.21139	293.15	293.15	0	336.267	336.267	0.07629	0.0763665

199	63.46	-74.2196	20.0008	-0.0999906	1.20868	293.15	293.15	0	336.44	336.44	0.0763336	0.0764091

200	63.64	-73.6548	20.0008	-0.0992241	1.2056	293.15	293.15	0	336.61	336.61	0.0763769	0.0764522

201	63.82	-73.0055	20.0008	-0.0983443	1.20749	293.15	293.15	0	336.778	336.778	0.0764189	0.0764928

202	63.99	-72.23	20.0008	-0.0972944	1.20355	293.15	293.15	0	336.951	336.951	0.076462	0.0765339

203	64.17	-71.3516	20.0008	-0.0961061	1.20208	293.15	293.15	0	337.099	337.099	0.0765035	0.0765746

204	64.34	-70.4383	20.0008	-0.0948709	1.20015	293.15	293.15	0	337.267	337.267	0.0765451	0.0766156

205	64.52	-69.5017	19.9935	-0.0936046	1.19804	293.15	293.15	0	337.436	337.436	0.0765878	0.0766564

206	64.68	-68.4875	19.9904	-0.0922341	1.19738	293.15	293.15	0	337.613	337.613	0.076629	0.0766949

207	64.85	-67.186	19.9904	-0.0904766	1.19352	293.15	293.15	0	337.783	337.783	0.0766699	0.0767342

208	65.02	-65.6772	19.9977	-0.0884402	1.18636	293.15	293.15	0	337.948	337.948	0.0767127	0.0767745

209	65.19	-63.9698	20.0008	-0.0861366	1.18302	293.15	293.15	0	338.103	338.103	0.0767548	0.0768142

210	65.36	-62.0937	20.0008	-0.083606	1.17619	293.15	293.15	0	338.269	338.269	0.0767977	0.0768544

211	65.53	-60.2727	20.0008	-0.0811501	1.16987	293.15	293.15	0	338.442	338.442	0.0768392	0.0768934

212	65.69	-58.2421	20.0008	-0.0784121	1.16213	293.15	293.15	0	338.614	338.614	0.0768808	0.0769317

213	65.86	-56.1329	20.0008	-0.0755687	1.15745	293.15	293.15	0	338.779	338.779	0.0769219	0.076971

214	66.03	-54.0409	19.9946	-0.0727488	1.14822	293.15	293.15	0	338.942	338.942	0.0769642	0.0770098

215	66.19	-51.1362	19.9956	-0.0688351	1.12917	293.15	293.15	0	339.107	339.107	0.0770101	0.0770485

216	66.37	-47.2553	20.0008	-0.0636076	1.10794	293.15	293.15	0	339.272	339.272	0.0770576	0.077089

217	66.54	-42.472	20.0008	-0.057166	1.08415	293.15	293.15	0	339.445	339.445	0.0771071	0.07713

218	66.72	-37.3547	19.9956	-0.0502756	1.05849	293.15	293.15	0	339.618	339.618	0.0771546	0.0771715

219	66.89	-32.3701	20.0008	-0.0435647	1.03942	293.15	293.15	0	339.783	339.783	0.0771989	0.0772099

220	67.04	-27.7745	20.0008	-0.0373781	1.02384	293.15	293.15	0	339.937	339.937	0.0772404	0.0772456

221	67.18	-23.7819	20.0008	-0.0320034	1.01659	293.15	293.15	0	340.111	340.111	0.0772782	0.0772797

222	67.32	-20.4301	20.0008	-0.0274918	1.01477	293.15	293.15	0	340.285	340.285	0.0773135	0.077312

223	67.46	-17.6838	20.0008	-0.0237952	1.0139	293.15	293.15	0	340.439	340.439	0.0773473	0.0773442

224	67.6	-15.5046	20.0008	-0.0208621	1.01345	293.15	293.15	0	340.606	340.606	0.0773807	0.0773763

225	67.73	-13.848	20.0008	-0.0186322	1.01855	293.15	293.15	0	340.779	340.779	0.0774131	0.0774073

226	67.87	-12.6402	19.9977	-0.0170065	1.0248	293.15	293.15	0	340.948	340.948	0.0774446	0.0774386

227	68	-11.7467	19.9977	-0.0158037	1.03008	293.15	293.15	0	341.1	341.1	0.0774772	0.077471

228	68.14	-11.1489	19.9935	-0.0149989	1.03601	293.15	293.15	0	341.274	341.274	0.0775095	0.0775032

229	68.28	-10.7299	19.9925	-0.0144345	1.04578	293.15	293.15	0	341.438	341.438	0.0775427	0.0775363

230	68.43	-10.4417	20.0008	-0.0140462	1.05173	293.15	293.15	0	341.606	341.606	0.0775766	0.0775698

231	68.57	-10.2876	20.0008	-0.0138382	1.05953	293.15	293.15	0	341.775	341.775	0.0776107	0.0776041

232	68.72	-10.2293	20.0029	-0.0137593	1.06932	293.15	293.15	0	341.948	341.948	0.077645	0.0776388

233	68.88	-10.2308	20.005	-0.0137606	1.0763	293.15	293.15	0	342.097	342.097	0.0776799	0.0776744

234	69.03	-10.2518	20.0008	-0.0137883	1.08424	293.15	293.15	0	342.269	342.269	0.0777161	0.0777102

235	69.19	-10.2676	20.0008	-0.0138088	1.08986	293.15	293.15	0	342.442	342.442	0.0777525	0.0777474

236	69.35	-10.278	20.0008	-0.0138222	1.09351	293.15	293.15	0	342.607	342.607	0.0777894	0.0777845

237	69.51	-10.2876	20.0008	-0.0138344	1.10384	293.15	293.15	0	342.779	342.779	0.0778265	0.0778224

238	69.67	-10.3626	20.0008	-0.0139345	1.11023	293.15	293.15	0	342.946	342.946	0.0778629	0.077859

239	69.83	-10.5562	20.0008	-0.0141942	1.1137	293.15	293.15	0	343.1	343.1	0.0779013	0.0778979

240	70	-10.6995	19.9956	-0.0143861	1.11537	293.15	293.15	0	343.273	343.273	0.0779401	0.0779364

241	70.16	-10.8047	19.9904	-0.0145269	1.11994	293.15	293.15	0	343.437	343.437	0.077978	0.0779739

242	70.32	-10.8839	19.9956	-0.0146326	1.12923	293.15	293.15	0	343.61	343.61	0.0780159	0.0780119

243	70.49	-10.9602	19.9956	-0.0147344	1.13423	293.15	293.15	0	343.775	343.775	0.078054	0.0780512

244	70.66	-10.988	20.0008	-0.0147711	1.13627	293.15	293.15	0	343.947	343.947	0.078093	0.0780907

245	70.83	-11.0236	20.0008	-0.0148183	1.14304	293.15	293.15	0	344.103	344.103	0.0781319	0.0781297

246	70.99	-11.0061	19.9966	-0.014794	1.14621	293.15	293.15	0	344.268	344.268	0.0781704	0.0781672

247	71.16	-10.9943	19.9998	-0.0147773	1.1525	293.15	293.15	0	344.442	344.442	0.078209	0.0782068

248	71.33	-11.0083	20.0008	-0.0147954	1.15786	293.15	293.15	0	344.613	344.613	0.0782476	0.078246

249	71.49	-11.0412	20.0008	-0.0148389	1.16352	293.15	293.15	0	344.778	344.778	0.0782861	0.0782847

250	71.66	-11.0541	19.9914	-0.0148555	1.16867	293.15	293.15	0	344.944	344.944	0.0783252	0.0783242

251	71.83	-11.0179	19.9904	-0.0148061	1.1713	293.15	293.15	0	345.101	345.101	0.0783642	0.0783625

252	72	-11.0195	19.9904	-0.0148076	1.17557	293.15	293.15	0	345.27	345.27	0.0784029	0.0784019

253	72.17	-11.0098	19.9987	-0.0147937	1.17914	293.15	293.15	0	345.445	345.445	0.0784423	0.0784417

254	72.33	-11.02	20.0008	-0.0148067	1.18504	293.15	293.15	0	345.615	345.615	0.0784808	0.0784805

255	72.5	-11.0848	20.0008	-0.014893	1.18846	293.15	293.15	0	345.783	345.783	0.078519	0.0785192

256	72.67	-11.1526	19.9925	-0.0149833	1.19216	293.15	293.15	0	345.938	345.938	0.0785572	0.0785582

257	72.84	-11.2093	19.9925	-0.0150587	1.19892	293.15	293.15	0	346.104	346.104	0.0785969	0.0785978

258	73.01	-11.2587	20.0008	-0.0151243	1.20224	293.15	293.15	0	346.272	346.272	0.0786361	0.078637

259	73.17	-11.2519	20.0008	-0.0151145	1.2043	293.15	293.15	0	346.441	346.441	0.078676	0.078676

260	73.34	-11.2799	20.0008	-0.0151513	1.21016	293.15	293.15	0	346.61	346.61	0.0787147	0.0787145

261	73.51	-11.2724	19.9946	-0.0151404	1.21451	293.15	293.15	0	346.773	346.773	0.0787528	0.0787532

262	73.68	-11.2391	19.9956	-0.0150949	1.21691	293.15	293.15	0	346.936	346.936	0.0787923	0.0787935

263	73.84	-11.2229	19.9904	-0.0150723	1.22407	293.15	293.15	0	347.108	347.108	0.0788307	0.0788319

264	74.01	-11.2176	19.9966	-0.0150645	1.22682	293.15	293.15	0	347.274	347.274	0.0788693	0.0788697

265	74.18	-11.2251	20.0008	-0.0150738	1.23224	293.15	293.15	0	347.446	347.446	0.0789085	0.0789093

266	74.34	-11.2172	19.9946	-0.0150626	1.23833	293.15	293.15	0	347.612	347.612	0.0789466	0.0789481

267	74.51	-11.1397	19.9956	-0.0149577	1.2406	293.15	293.15	0	347.767	347.767	0.0789855	0.0789863

268	74.67	-11.0923	20.0008	-0.0148933	1.24413	293.15	293.15	0	347.939	347.939	0.0790235	0.0790253

269	74.84	-11.1097	20.0008	-0.0149159	1.24705	293.15	293.15	0	348.113	348.113	0.0790626	0.0790641

270	75.01	-11.1528	20.0008	-0.0149731	1.25438	293.15	293.15	0	348.277	348.277	0.0791017	0.0791032

271	75.18	-11.2419	20.0008	-0.0150919	1.25717	293.15	293.15	0	348.441	348.441	0.0791405	0.0791423

272	75.35	-11.2944	19.9904	-0.0151615	1.26083	293.15	293.15	0	348.607	348.607	0.0791793	0.0791814

273	75.51	-11.2577	19.9904	-0.0151116	1.26868	293.15	293.15	0	348.769	348.769	0.0792178	0.0792198

274	75.68	-11.1836	19.9904	-0.0150114	1.27208	293.15	293.15	0	348.935	348.935	0.0792565	0.0792593

275	75.85	-11.1151	19.9998	-0.0149187	1.27639	293.15	293.15	0	349.109	349.109	0.0792955	0.0792978

276	76.01	-11.0847	20.0008	-0.0148771	1.28178	293.15	293.15	0	349.28	349.28	0.0793338	0.0793365

277	76.18	-11.0754	20.0008	-0.0148639	1.28485	293.15	293.15	0	349.446	349.446	0.0793732	0.0793758

278	76.35	-11.1013	20.0008	-0.0148978	1.29298	293.15	293.15	0	349.612	349.612	0.0794116	0.0794148

279	76.52	-11.0765	20.0008	-0.0148638	1.29398	293.15	293.15	0	349.772	349.772	0.0794513	0.079454

280	76.68	-11.0033	19.9925	-0.0147649	1.29772	293.15	293.15	0	349.939	349.939	0.0794894	0.0794925

281	76.84	-10.9721	19.9987	-0.0147222	1.30491	293.15	293.15	0	350.112	350.112	0.0795268	0.0795297

282	77.01	-10.9873	19.9977	-0.0147419	1.30977	293.15	293.15	0	350.283	350.283	0.0795661	0.0795687

283	77.18	-11.0229	19.9987	-0.014789	1.31161	293.15	293.15	0	350.45	350.45	0.0796053	0.0796089

284	77.35	-11.0178	20.0008	-0.0147814	1.31753	293.15	293.15	0	350.619	350.619	0.0796439	0.0796476

285	77.52	-11.0072	20.0008	-0.0147664	1.32015	293.15	293.15	0	350.78	350.78	0.0796835	0.0796878

286	77.69	-11.0114	20.0008	-0.0147712	1.32979	293.15	293.15	0	350.946	350.946	0.0797215	0.0797264

287	77.85	-10.988	20.0008	-0.0147391	1.33289	293.15	293.15	0	351.101	351.101	0.0797598	0.0797643

288	78.02	-10.9789	20.0008	-0.0147262	1.33607	293.15	293.15	0	351.266	351.266	0.0797987	0.0798034

289	78.19	-10.9909	19.9946	-0.0147415	1.33827	293.15	293.15	0	351.438	351.438	0.0798375	0.0798427

290	78.36	-10.9771	19.9966	-0.0147222	1.34461	293.15	293.15	0	351.611	351.611	0.0798772	0.079882

291	78.52	-11.0294	20.0008	-0.0147917	1.34932	293.15	293.15	0	351.758	351.758	0.0799145	0.0799195

292	78.69	-10.9943	20.0008	-0.0147439	1.35205	293.15	293.15	0	351.941	351.941	0.0799533	0.0799583

293	78.86	-10.9185	20.0008	-0.0146415	1.35645	293.15	293.15	0	352.105	352.105	0.0799931	0.0799979

294	79.03	-10.8952	20.0008	-0.0146095	1.3622	293.15	293.15	0	352.278	352.278	0.0800317	0.0800369

295	79.19	-10.906	20.0008	-0.0146233	1.36798	293.15	293.15	0	352.442	352.442	0.0800695	0.0800749

296	79.36	-10.8988	19.9966	-0.0146129	1.36862	293.15	293.15	0	352.607	352.607	0.0801081	0.080114

297	79.53	-10.9233	19.9998	-0.0146449	1.37229	293.15	293.15	0	352.764	352.764	0.0801476	0.080154

298	79.69	-10.9695	20.0008	-0.0147062	1.38157	293.15	293.15	0	352.944	352.944	0.0801857	0.0801921

299	79.86	-11.0048	20.0008	-0.0147528	1.38498	293.15	293.15	0	353.109	353.109	0.0802248	0.0802304

300	80.03	-10.9641	19.9914	-0.0146975	1.39018	293.15	293.15	0	353.283	353.283	0.0802634	0.0802696

301	80.19	-10.8789	19.9987	-0.0145825	1.39595	293.15	293.15	0	353.446	353.446	0.080302	0.0803083

302	80.36	-10.8058	20.0019	-0.0144837	1.4003	293.15	293.15	0	353.609	353.609	0.0803404	0.080347

303	80.53	-10.832	20.0008	-0.0145181	1.40379	293.15	293.15	0	353.767	353.767	0.0803792	0.0803853

304	80.69	-10.8905	19.9977	-0.0145959	1.40853	293.15	293.15	0	353.941	353.941	0.0804179	0.0804243

305	80.86	-10.858	19.9987	-0.0145516	1.41406	293.15	293.15	0	354.11	354.11	0.0804549	0.0804638

306	81.03	-10.8277	19.9925	-0.0145103	1.42107	293.15	293.15	0	354.278	354.278	0.0804941	0.0805019

307	81.2	-10.8565	19.9925	-0.0145481	1.42412	293.15	293.15	0	354.435	354.435	0.0805327	0.080541

308	81.37	-10.9568	20.0008	-0.0146818	1.42635	293.15	293.15	0	354.602	354.602	0.0805727	0.0805812

309	81.53	-10.994	20.0008	-0.0147308	1.43232	293.15	293.15	0	354.772	354.772	0.0806109	0.0806191

310	81.71	-10.9506	19.9987	-0.014672	1.43825	293.15	293.15	0	354.945	354.945	0.08065	0.0806591

311	81.87	-10.8553	19.9977	-0.0145435	1.44172	293.15	293.15	0	355.113	355.113	0.0806891	0.0806977

312	82.04	-10.7454	20.0008	-0.0143956	1.4464	293.15	293.15	0	355.274	355.274	0.0807269	0.0807355

313	82.2	-10.6719	20.0008	-0.0142963	1.44809	293.15	293.15	0	355.44	355.44	0.0807662	0.0807744

314	82.37	-10.651	20.0008	-0.0142676	1.45565	293.15	293.15	0	355.605	355.605	0.0808046	0.0808132

315	82.54	-10.7266	20.0008	-0.0143682	1.46109	293.15	293.15	0	355.776	355.776	0.0808431	0.0808523

316	82.7	-10.7634	20.0008	-0.0144167	1.46303	293.15	293.15	0	355.95	355.95	0.0808819	0.0808907

317	82.87	-10.7186	20.0008	-0.0143561	1.46615	293.15	293.15	0	356.097	356.097	0.080921	0.080929

318	83.03	-10.6589	20.0008	-0.0142754	1.47256	293.15	293.15	0	356.271	356.271	0.080958	0.0809672

319	83.21	-10.5789	19.9904	-0.0141676	1.47836	293.15	293.15	0	356.443	356.443	0.0809976	0.0810069

320	83.37	-10.5207	19.9956	-0.0140888	1.48263	293.15	293.15	0	356.608	356.608	0.0810357	0.0810445

321	83.54	-10.5008	20.0008	-0.0140616	1.49044	293.15	293.15	0	356.781	356.781	0.0810732	0.0810833

322	83.71	-10.5182	19.9904	-0.0140841	1.49279	293.15	293.15	0	356.945	356.945	0.0811125	0.0811229

323	83.87	-10.5472	19.9946	-0.0141222	1.49852	293.15	293.15	0	357.102	357.102	0.0811514	0.0811614

324	84.04	-10.5926	20.0008	-0.0141823	1.50324	293.15	293.15	0	357.275	357.275	0.0811903	0.0812011

325	84.21	-10.6049	19.9914	-0.0141981	1.50622	293.15	293.15	0	357.439	357.439	0.0812288	0.0812394

326	84.38	-10.6061	19.9946	-0.0141989	1.51324	293.15	293.15	0	357.61	357.61	0.0812675	0.0812791

327	84.55	-10.6422	19.9914	-0.0142466	1.51597	293.15	293.15	0	357.776	357.776	0.0813069	0.0813181

328	84.72	-10.7212	19.9998	-0.0143515	1.5237	293.15	293.15	0	357.943	357.943	0.0813449	0.0813569

329	84.88	-10.7363	20.0008	-0.0143711	1.52494	293.15	293.15	0	358.103	358.103	0.0813839	0.0813948

330	85.05	-10.7149	20.0091	-0.0143417	1.53045	293.15	293.15	0	358.27	358.27	0.0814227	0.081434

331	85.21	-10.6282	20.0029	-0.0142249	1.53671	293.15	293.15	0	358.443	358.443	0.0814601	0.0814722

332	85.38	-10.5746	20.0008	-0.0141525	1.54014	293.15	293.15	0	358.613	358.613	0.0814992	0.0815107

333	85.55	-10.6254	20.0008	-0.0142197	1.54254	293.15	293.15	0	358.781	358.781	0.0815382	0.0815492

334	85.71	-10.6344	20.0008	-0.0142311	1.54878	293.15	293.15	0	358.947	358.947	0.0815766	0.0815879

335	85.88	-10.6366	20.0008	-0.0142334	1.55567	293.15	293.15	0	359.102	359.102	0.0816145	0.0816264

336	86.05	-10.6557	19.9935	-0.0142582	1.55933	293.15	293.15	0	359.269	359.269	0.0816534	0.0816659

337	86.22	-10.6634	19.9977	-0.0142678	1.56462	293.15	293.15	0	359.448	359.448	0.0816923	0.0817044

338	86.38	-10.6394	20.0008	-0.0142349	1.57149	293.15	293.15	0	359.616	359.616	0.0817311	0.0817434

339	86.55	-10.566	20.0008	-0.0141361	1.5736	293.15	293.15	0	359.785	359.785	0.0817703	0.0817827

340	86.72	-10.4815	20.0008	-0.0140223	1.57744	293.15	293.15	0	359.933	359.933	0.0818083	0.0818201

341	86.88	-10.3875	19.9946	-0.0138959	1.58308	293.15	293.15	0	360.106	360.106	0.0818458	0.0818578

342	87.05	-10.3964	19.9966	-0.0139071	1.59033	293.15	293.15	0	360.272	360.272	0.0818848	0.0818971

343	87.22	-10.4608	20.0008	-0.0139924	1.59293	293.15	293.15	0	360.437	360.437	0.0819229	0.081936

344	87.38	-10.4811	20.0008	-0.0140189	1.59868	293.15	293.15	0	360.61	360.61	0.0819615	0.0819745

345	87.55	-10.4868	20.0008	-0.0140259	1.60168	293.15	293.15	0	360.773	360.773	0.0820007	0.0820139

346	87.72	-10.4601	20.0008	-0.0139894	1.60455	293.15	293.15	0	360.946	360.946	0.0820393	0.0820526

347	87.88	-10.4189	20.0008	-0.0139336	1.60934	293.15	293.15	0	361.103	361.103	0.0820783	0.0820908

348	88.05	-10.4318	20.0008	-0.0139502	1.61784	293.15	293.15	0	361.274	361.274	0.0821164	0.0821295

349	88.22	-10.4226	20.0008	-0.0139371	1.6222	293.15	293.15	0	361.441	361.441	0.0821549	0.0821674

350	88.38	-10.381	19.9914	-0.0138808	1.62783	293.15	293.15	0	361.613	361.613	0.0821929	0.0822061

351	88.55	-10.3643	19.9946	-0.0138578	1.63361	293.15	293.15	0	361.777	361.777	0.0822318	0.082245

352	88.72	-10.3157	20.0008	-0.0137922	1.63868	293.15	293.15	0	361.949	361.949	0.0822701	0.0822831

353	88.89	-10.213	20.0008	-0.0136542	1.64226	293.15	293.15	0	362.099	362.099	0.0823091	0.0823224

354	89.05	-10.1643	20.0008	-0.0135884	1.6458	293.15	293.15	0	362.271	362.271	0.0823479	0.0823613

355	89.22	-10.1694	20.0008	-0.0135945	1.65279	293.15	293.15	0	362.441	362.441	0.0823861	0.0823996

356	89.39	-10.1409	20.0008	-0.0135558	1.65801	293.15	293.15	0	362.609	362.609	0.0824239	0.0824385

357	89.55	-10.1665	20.0008	-0.0135893	1.6622	293.15	293.15	0	362.782	362.782	0.0824623	0.0824766

358	89.72	-10.2177	20.0008	-0.013657	1.66637	293.15	293.15	0	362.942	362.942	0.0825013	0.0825158

359	89.89	-10.3445	20.0008	-0.0138259	1.67212	293.15	293.15	0	363.103	363.103	0.0825395	0.082554

360	90.05	-10.4608	20.0008	-0.0139806	1.67818	293.15	293.15	0	363.276	363.276	0.0825784	0.0825924

361	90.22	-10.4898	20.0008	-0.0140186	1.6816	293.15	293.15	0	363.44	363.44	0.0826167	0.0826312

362	90.39	-10.4182	19.9987	-0.0139222	1.68649	293.15	293.15	0	363.608	363.608	0.0826557	0.0826706

363	90.55	-10.3138	19.9904	-0.013782	1.6933	293.15	293.15	0	363.777	363.777	0.0826939	0.0827084

364	90.72	-10.2193	19.9977	-0.0136551	1.69975	293.15	293.15	0	363.944	363.944	0.0827323	0.0827473

365	90.89	-10.1603	20.0008	-0.0135756	1.70237	293.15	293.15	0	364.108	364.108	0.0827712	0.0827863

366	91.06	-10.1392	20.0008	-0.0135467	1.70766	293.15	293.15	0	364.271	364.271	0.0828095	0.0828251

367	91.23	-10.1689	19.9946	-0.0135857	1.71271	293.15	293.15	0	364.444	364.444	0.0828484	0.0828639

368	91.4	-10.2505	19.9966	-0.013694	1.71577	293.15	293.15	0	364.61	364.61	0.0828874	0.0829033

369	91.56	-10.2535	20.0008	-0.0136974	1.72147	293.15	293.15	0	364.782	364.782	0.0829248	0.0829408

370	91.72	-10.1697	20.0008	-0.0135847	1.72586	293.15	293.15	0	364.948	364.948	0.0829629	0.0829787

371	91.89	-10.1024	20.0008	-0.0134941	1.73409	293.15	293.15	0	365.103	365.103	0.0830015	0.083018

372	92.06	-10.0931	20.0008	-0.013481	1.73757	293.15	293.15	0	365.276	365.276	0.0830405	0.0830573

373	92.23	-10.1053	20.0008	-0.0134966	1.74054	293.15	293.15	0	365.44	365.44	0.0830792	0.0830956

374	92.4	-10.1666	20.0008	-0.0135779	1.74392	293.15	293.15	0	365.613	365.613	0.0831174	0.083134

375	92.57	-10.213	20.0008	-0.0136391	1.75191	293.15	293.15	0	365.777	365.777	0.0831566	0.0831735

376	92.73	-10.1967	20.0008	-0.0136167	1.75816	293.15	293.15	0	365.943	365.943	0.0831942	0.0832111

377	92.9	-10.1051	20.0008	-0.0134937	1.75967	293.15	293.15	0	366.098	366.098	0.0832331	0.08325

378	93.07	-10.0307	20.0008	-0.0133936	1.7658	293.15	293.15	0	366.269	366.269	0.0832722	0.083289

379	93.23	-9.94325	20.0008	-0.0132762	1.77358	293.15	293.15	0	366.444	366.444	0.0833096	0.0833265

380	93.4	-9.88611	20.0008	-0.0131993	1.77762	293.15	293.15	0	366.608	366.608	0.0833481	0.0833651

381	93.56	-9.91735	20.0008	-0.0132403	1.78415	293.15	293.15	0	366.78	366.78	0.083386	0.0834038

382	93.73	-9.97099	20.0008	-0.0133112	1.78735	293.15	293.15	0	366.937	366.937	0.0834248	0.0834433

383	93.9	-10.0321	20.0008	-0.0133922	1.79448	293.15	293.15	0	367.102	367.102	0.0834634	0.0834814

384	94.07	-10.0502	20.0008	-0.0134157	1.79823	293.15	293.15	0	367.271	367.271	0.0835023	0.0835206

385	94.24	-9.99622	20.0008	-0.0133429	1.80134	293.15	293.15	0	367.439	367.439	0.083541	0.083559

386	94.4	-9.92812	20.0008	-0.0132513	1.80864	293.15	293.15	0	367.612	367.612	0.0835789	0.0835979

387	94.57	-9.82769	20.0008	-0.0131166	1.81324	293.15	293.15	0	367.783	367.783	0.0836181	0.0836363

388	94.74	-9.76633	20.0008	-0.0130341	1.8157	293.15	293.15	0	367.941	367.941	0.0836568	0.0836758

389	94.91	-9.77702	20.0008	-0.0130477	1.82153	293.15	293.15	0	368.098	368.098	0.0836943	0.0837136

390	95.07	-9.80813	19.9935	-0.0130886	1.82803	293.15	293.15	0	368.271	368.271	0.0837323	0.0837525

391	95.24	-9.80557	19.9904	-0.0130845	1.83367	293.15	293.15	0	368.438	368.438	0.0837708	0.0837906

392	95.41	-9.85278	19.9977	-0.0131468	1.83898	293.15	293.15	0	368.608	368.608	0.0838096	0.0838291

393	95.57	-9.90626	20.0008	-0.0132175	1.84759	293.15	293.15	0	368.783	368.783	0.083847	0.0838676

394	95.74	-9.90093	19.9935	-0.0132098	1.84989	293.15	293.15	0	368.94	368.94	0.0838865	0.0839068

395	95.91	-9.86861	19.9966	-0.013166	1.85462	293.15	293.15	0	369.102	369.102	0.0839257	0.083946

396	96.08	-9.88449	20.0008	-0.0131865	1.85833	293.15	293.15	0	369.275	369.275	0.0839637	0.0839839

397	96.24	-9.87795	20.0008	-0.0131771	1.86564	293.15	293.15	0	369.441	369.441	0.0840012	0.0840221

398	96.41	-9.86024	20.0008	-0.0131528	1.8731	293.15	293.15	0	369.612	369.612	0.0840398	0.0840606

399	96.58	-9.77564	20.0071	-0.0130393	1.87497	293.15	293.15	0	369.785	369.785	0.0840792	0.0840992

400	96.75	-9.68209	20.005	-0.0129139	1.87934	293.15	293.15	0	369.942	369.942	0.0841178	0.0841381

401	96.91	-9.68715	20.0008	-0.01292	1.88762	293.15	293.15	0	370.106	370.106	0.0841544	0.0841754

402	97.08	-9.70528	20.0008	-0.0129435	1.88972	293.15	293.15	0	370.27	370.27	0.0841929	0.0842145

403	97.25	-9.72164	20.0008	-0.0129647	1.8971	293.15	293.15	0	370.444	370.444	0.0842328	0.0842539

404	97.41	-9.72917	20.0008	-0.0129741	1.89945	293.15	293.15	0	370.607	370.607	0.0842711	0.0842923

405	97.58	-9.68899	20.0008	-0.0129199	1.90336	293.15	293.15	0	370.781	370.781	0.0843097	0.084331

406	97.74	-9.65967	20.0008	-0.0128801	1.91113	293.15	293.15	0	370.945	370.945	0.0843477	0.0843686

407	97.91	-9.64739	20.0008	-0.0128631	1.91675	293.15	293.15	0	371.111	371.111	0.0843864	0.0844073

408	98.08	-9.57756	19.9914	-0.0127694	1.92155	293.15	293.15	0	371.273	371.273	0.0844249	0.0844456

409	98.25	-9.52408	19.9987	-0.0126974	1.92527	293.15	293.15	0	371.441	371.441	0.0844636	0.0844845

410	98.42	-9.50962	20.0008	-0.0126775	1.93014	293.15	293.15	0	371.61	371.61	0.0845014	0.0845232

411	98.58	-9.49463	20.0008	-0.0126569	1.93827	293.15	293.15	0	371.778	371.778	0.08454	0.0845618

412	98.75	-9.47067	20.0008	-0.0126243	1.94175	293.15	293.15	0	371.942	371.942	0.0845783	0.0845995

413	98.91	-9.43252	20.0008	-0.0125729	1.94609	293.15	293.15	0	372.099	372.099	0.0846162	0.0846378

414	99.08	-9.37354	20.0008	-0.0124936	1.95196	293.15	293.15	0	372.267	372.267	0.0846542	0.0846757

415	99.25	-9.30866	20.0008	-0.0124065	1.95818	293.15	293.15	0	372.436	372.436	0.0846923	0.0847147

416	99.41	-9.28537	20.0008	-0.0123749	1.96678	293.15	293.15	0	372.613	372.613	0.0847305	0.0847525

417	99.58	-9.30623	20.0008	-0.012402	1.96963	293.15	293.15	0	372.783	372.783	0.0847691	0.0847919

418	99.75	-9.31687	20.0008	-0.0124156	1.97797	293.15	293.15	0	372.938	372.938	0.0848069	0.08483

419	99.91	-9.28274	20.0008	-0.0123695	1.97848	293.15	293.15	0	373.094	373.094	0.0848458	0.0848684

420	100.08	-9.26362	20.0008	-0.0123434	1.89699	293.15	293.15	0	373.051	373.051	0.084884	0.0849063

421	100.21	-9.32877	19.9946	-0.0124297	1.76544	293.15	293.15	0	372.88	372.88	0.0849136	0.084936

422	100.25	-8.96556	19.9966	-0.0119456	1.65326	293.15	293.15	0	372.707	372.707	0.0849263	0.0849458

423	100.22	-7.6604	20.0008	-0.0102068	1.57373	293.15	293.15	0	372.559	372.559	0.0849232	0.0849387

424	100.13	-5.6867	20.0008	-0.0075772	1.4959	293.15	293.15	0	372.385	372.385	0.0849072	0.0849181

425	100	-3.27345	20.0008	-0.00436185	1.43671	293.15	293.15	0	372.212	372.212	0.0848809	0.0848875

426	99.83	-0.620893	20.0008	-0.000827377	1.38805	293.15	293.15	0	372.039	372.039	0.0848471	0.0848497

427	99.63	2.13276	20.0008	0.0028422	1.35425	293.15	293.15	0	371.876	371.876	0.0848048	0.0848039

428	99.42	4.72665	19.9904	0.00629932	1.32992	293.15	293.15	0	371.712	371.712	0.0847592	0.0847553

429	99.2	7.18226	19.9946	0.00957261	1.31423	293.15	293.15	0	371.555	371.555	0.0847107	0.0847038

430	98.97	9.33954	20.0008	0.0124487	1.29721	293.15	293.15	0	371.381	371.381	0.0846601	0.0846511

431	98.74	11.1406	19.9914	0.0148504	1.28735	293.15	293.15	0	371.217	371.217	0.0846087	0.0845972

432	98.51	12.5033	19.9946	0.0166681	1.28261	293.15	293.15	0	371.046	371.046	0.0845564	0.0845441

433	98.27	13.5639	20.0008	0.0180831	1.27797	293.15	293.15	0	370.87	370.87	0.0845028	0.0844896

434	98.04	14.373	20.0102	0.0191631	1.28087	293.15	293.15	0	370.709	370.709	0.0844507	0.0844366

435	97.81	14.9592	20.0081	0.0199461	1.2796	293.15	293.15	0	370.55	370.55	0.084399	0.0843846

436	97.6	15.254	20.0008	0.0203405	1.2788	293.15	293.15	0	370.386	370.386	0.0843501	0.0843352

437	97.38	15.3832	20.0008	0.0205141	1.28368	293.15	293.15	0	370.213	370.213	0.0842992	0.0842852

438	97.18	15.4086	20.0008	0.0205492	1.28687	293.15	293.15	0	370.043	370.043	0.0842519	0.0842376

439	96.97	15.3598	20.0008	0.0204854	1.28444	293.15	293.15	0	369.875	369.875	0.0842042	0.0841904

440	96.78	15.2246	20.0008	0.0203063	1.28809	293.15	293.15	0	369.702	369.702	0.0841582	0.0841452

441	96.58	14.9998	20.0008	0.0200076	1.29067	293.15	293.15	0	369.538	369.538	0.0841132	0.0840999

442	96.38	14.7471	20.0008	0.0196717	1.29143	293.15	293.15	0	369.378	369.378	0.0840681	0.0840548

443	96.2	14.5191	19.9935	0.0193686	1.2905	293.15	293.15	0	369.218	369.218	0.0840258	0.084013

444	96.02	14.2734	19.9977	0.0190419	1.28779	293.15	293.15	0	369.044	369.044	0.0839835	0.0839707

445	95.84	14.0505	20.0008	0.0187455	1.28862	293.15	293.15	0	368.876	368.876	0.083941	0.0839288

446	95.67	13.8146	20.0008	0.0184318	1.28451	293.15	293.15	0	368.706	368.706	0.083901	0.0838888

447	95.49	13.5981	20.0008	0.0181439	1.28131	293.15	293.15	0	368.55	368.55	0.0838607	0.0838476

448	95.31	13.4032	20.0008	0.0178848	1.28065	293.15	293.15	0	368.384	368.384	0.0838197	0.0838077

449	95.14	13.1936	20.0008	0.017606	1.27919	293.15	293.15	0	368.213	368.213	0.0837802	0.0837682

450	94.97	12.9881	20.0008	0.0173326	1.27428	293.15	293.15	0	368.04	368.04	0.0837414	0.0837291

451	94.8	12.756	20.0008	0.0170238	1.27083	293.15	293.15	0	367.876	367.876	0.083702	0.08369

452	94.63	12.5605	20.0008	0.0167636	1.26832	293.15	293.15	0	367.71	367.71	0.0836626	0.083651

453	94.47	12.4573	20.0008	0.0166267	1.26404	293.15	293.15	0	367.555	367.555	0.083624	0.0836123

454	94.3	12.373	20.0008	0.0165151	1.26043	293.15	293.15	0	367.381	367.381	0.0835858	0.0835742

455	94.13	12.2718	20.0008	0.0163809	1.25406	293.15	293.15	0	367.218	367.218	0.0835467	0.0835349

456	93.97	12.1869	20.0008	0.0162683	1.2471	293.15	293.15	0	367.045	367.045	0.0835094	0.0834975

457	93.8	12.1037	20.0008	0.0161581	1.24593	293.15	293.15	0	366.871	366.871	0.083471	0.0834585

458	93.64	12.0183	20.0008	0.0160448	1.24364	293.15	293.15	0	366.716	366.716	0.083432	0.0834204

459	93.47	11.9717	20.0008	0.0159834	1.23574	293.15	293.15	0	366.55	366.55	0.0833945	0.0833821

460	93.3	11.9732	20.0008	0.0159862	1.23047	293.15	293.15	0	366.379	366.379	0.083355	0.0833426

461	93.13	11.9974	20.0008	0.0160194	1.22442	293.15	293.15	0	366.212	366.212	0.0833165	0.0833039

462	92.97	12.0028	20.0008	0.0160273	1.21824	293.15	293.15	0	366.04	366.04	0.0832784	0.0832659

463	92.8	11.9564	20.0008	0.0159662	1.21219	293.15	293.15	0	365.868	365.868	0.0832405	0.0832279

464	92.64	11.8956	19.9914	0.0158858	1.20984	293.15	293.15	0	365.696	365.696	0.0832024	0.0831897

465	92.47	11.8379	19.9977	0.0158096	1.20598	293.15	293.15	0	365.553	365.553	0.0831636	0.0831507

466	92.3	11.8352	19.9935	0.0158068	1.20104	293.15	293.15	0	365.386	365.386	0.0831254	0.0831122

467	92.13	11.8379	19.9966	0.0158112	1.19731	293.15	293.15	0	365.214	365.214	0.0830867	0.0830732

468	91.96	11.8851	20.0008	0.015875	1.18867	293.15	293.15	0	365.048	365.048	0.083048	0.0830339

469	91.79	11.9293	20.0008	0.0159348	1.18487	293.15	293.15	0	364.877	364.877	0.0830095	0.0829952

470	91.63	11.9255	19.9946	0.0159306	1.18061	293.15	293.15	0	364.712	364.712	0.0829715	0.082957

471	91.46	11.9513	19.9956	0.0159659	1.17732	293.15	293.15	0	364.556	364.556	0.0829332	0.0829186

472	91.3	11.932	20.0008	0.0159408	1.17462	293.15	293.15	0	364.383	364.383	0.0828939	0.0828797

473	91.13	11.8797	20.0008	0.0158718	1.16516	293.15	293.15	0	364.21	364.21	0.0828559	0.0828408

474	90.96	11.8658	20.0008	0.0158541	1.1639	293.15	293.15	0	364.046	364.046	0.0828172	0.0828019

475	90.79	11.8578	20.0008	0.0158441	1.16021	293.15	293.15	0	363.873	363.873	0.0827784	0.0827629

476	90.62	11.8833	19.9956	0.0158789	1.15668	293.15	293.15	0	363.699	363.699	0.0827388	0.0827244

477	90.45	11.9228	19.9946	0.0159326	1.15034	293.15	293.15	0	363.552	363.552	0.0827009	0.0826854

478	90.29	11.8946	20.0008	0.0158957	1.1441	293.15	293.15	0	363.379	363.379	0.0826628	0.0826469

479	90.13	11.8284	20.0008	0.015808	1.13987	293.15	293.15	0	363.213	363.213	0.0826246	0.0826093

480	89.95	11.7905	20.0008	0.0157582	1.13431	293.15	293.15	0	363.043	363.043	0.0825852	0.0825697

481	89.79	11.7567	19.9914	0.0157137	1.12838	293.15	293.15	0	362.877	362.877	0.0825471	0.0825311

482	89.62	11.7536	19.9935	0.0157104	1.12532	293.15	293.15	0	362.711	362.711	0.082508	0.0824925

483	89.45	11.756	20.0008	0.0157143	1.1209	293.15	293.15	0	362.551	362.551	0.0824704	0.0824536

484	89.29	11.7025	19.9925	0.0156436	1.11483	293.15	293.15	0	362.383	362.383	0.0824317	0.0824151

485	89.12	11.6662	19.9935	0.0155959	1.11146	293.15	293.15	0	362.21	362.21	0.0823919	0.0823759

486	88.95	11.635	19.9925	0.015555	1.10661	293.15	293.15	0	362.04	362.04	0.0823541	0.082338

487	88.78	11.5634	19.9987	0.01546	1.10394	293.15	293.15	0	361.873	361.873	0.0823153	0.0822991

488	88.62	11.5161	20.0008	0.0153975	1.09793	293.15	293.15	0	361.707	361.707	0.0822773	0.0822606

489	88.45	11.5313	20.0008	0.0154186	1.09231	293.15	293.15	0	361.552	361.552	0.0822386	0.0822218

490	88.28	11.5721	19.9935	0.0154739	1.08876	293.15	293.15	0	361.384	361.384	0.0822001	0.0821829

491	88.11	11.6409	19.9904	0.0155667	1.08432	293.15	293.15	0	361.215	361.215	0.0821615	0.0821441

492	87.95	11.7229	19.9977	0.0156772	1.07914	293.15	293.15	0	361.042	361.042	0.0821223	0.0821049

493	87.78	11.7447	20.0008	0.0157072	1.07703	293.15	293.15	0	360.877	360.877	0.0820831	0.0820656

494	87.61	11.713	20.0008	0.0156655	1.07267	293.15	293.15	0	360.708	360.708	0.0820442	0.0820273

495	87.45	11.6812	20.0008	0.0156238	1.06861	293.15	293.15	0	360.548	360.548	0.0820062	0.0819894

496	87.28	11.6628	20.0008	0.0156	1.05751	293.15	293.15	0	360.382	360.382	0.0819686	0.081951

497	87.11	11.631	20.0008	0.0155582	1.05626	293.15	293.15	0	360.21	360.21	0.0819296	0.0819116

498	86.94	11.5782	20.0008	0.0154884	1.05116	293.15	293.15	0	360.045	360.045	0.081891	0.0818729

499	86.78	11.5026	20.0008	0.015388	1.0486	293.15	293.15	0	359.889	359.889	0.0818524	0.0818345

500	86.61	11.4797	20.0008	0.0153582	1.04563	293.15	293.15	0	359.717	359.717	0.0818138	0.0817957

501	86.44	11.4865	20.0008	0.0153681	1.03749	293.15	293.15	0	359.543	359.543	0.0817752	0.0817571

502	86.28	11.4582	19.9956	0.0153309	1.03421	293.15	293.15	0	359.379	359.379	0.0817371	0.0817184

503	86.1	11.3838	19.9904	0.0152322	1.02958	293.15	293.15	0	359.206	359.206	0.0816979	0.0816786

504	85.94	11.3526	19.9956	0.0151912	1.02752	293.15	293.15	0	359.033	359.033	0.0816585	0.0816399

505	85.77	11.4255	20.0008	0.0152895	1.02286	293.15	293.15	0	358.885	358.885	0.0816201	0.0816015

506	85.6	11.5148	19.9914	0.0154097	1.01662	293.15	293.15	0	358.712	358.712	0.0815817	0.0815628

507	85.44	11.4875	19.9946	0.015374	1.0123	293.15	293.15	0	358.547	358.547	0.0815431	0.0815239

508	85.27	11.4435	20.0008	0.0153158	1.00671	293.15	293.15	0	358.377	358.377	0.0815041	0.0814853

509	85.1	11.4295	20.0008	0.015298	1.00231	293.15	293.15	0	358.211	358.211	0.0814661	0.0814466

510	84.93	11.4444	20.0008	0.0153187	0.998155	293.15	293.15	0	358.044	358.044	0.0814267	0.0814069

511	84.76	11.4891	19.9925	0.0153792	0.995099	293.15	293.15	0	357.884	357.884	0.0813883	0.0813678

512	84.6	11.4621	19.9987	0.0153439	0.989224	293.15	293.15	0	357.717	357.717	0.0813497	0.0813295

513	84.43	11.4322	20.0008	0.0153046	0.984915	293.15	293.15	0	357.544	357.544	0.0813116	0.0812914

514	84.27	11.4375	20.0008	0.0153125	0.980847	293.15	293.15	0	357.374	357.374	0.081273	0.0812531

515	84.1	11.4756	20.0008	0.0153642	0.977457	293.15	293.15	0	357.222	357.222	0.081234	0.0812137

516	83.93	11.5179	20.0008	0.0154217	0.971874	293.15	293.15	0	357.048	357.048	0.0811957	0.0811754

517	83.77	11.4775	19.9935	0.0153684	0.967217	293.15	293.15	0	356.882	356.882	0.0811566	0.0811368

518	83.6	11.4165	19.9977	0.0152874	0.963724	293.15	293.15	0	356.712	356.712	0.081118	0.0810976

519	83.43	11.392	20.0008	0.0152554	0.956408	293.15	293.15	0	356.539	356.539	0.0810795	0.0810591

520	83.26	11.3806	20.0008	0.015241	0.950805	293.15	293.15	0	356.381	356.381	0.0810411	0.0810195

521	83.1	11.3403	19.9946	0.0151877	0.945953	293.15	293.15	0	356.219	356.219	0.0810024	0.0809817

522	82.93	11.2953	19.9966	0.0151282	0.943552	293.15	293.15	0	356.045	356.045	0.0809633	0.0809421

523	82.76	11.2613	20.0008	0.0150834	0.940215	293.15	293.15	0	355.878	355.878	0.0809246	0.0809033

524	82.59	11.2642	20.0008	0.015088	0.934545	293.15	293.15	0	355.708	355.708	0.0808862	0.080864

525	82.42	11.2312	20.0008	0.0150446	0.931275	293.15	293.15	0	355.535	355.535	0.0808472	0.0808253

526	82.25	11.2242	20.0008	0.0150361	0.928335	293.15	293.15	0	355.378	355.378	0.0808079	0.0807859

527	82.09	11.2698	19.9956	0.0150979	0.923978	293.15	293.15	0	355.214	355.214	0.0807696	0.0807474

528	81.91	11.2871	20.0008	0.0151218	0.923029	293.15	293.15	0	355.041	355.041	0.0807302	0.0807073

529	81.75	11.2794	20.0008	0.0151122	0.915309	293.15	293.15	0	354.877	354.877	0.0806919	0.0806698

530	81.59	11.2236	20.0008	0.0150382	0.910252	293.15	293.15	0	354.713	354.713	0.0806536	0.080631

531	81.42	11.1925	20.0008	0.0149973	0.903497	293.15	293.15	0	354.545	354.545	0.0806154	0.0805933

532	81.25	11.1372	20.0008	0.014924	0.898712	293.15	293.15	0	354.382	354.382	0.0805769	0.0805543

533	81.08	11.0994	20.0008	0.0148741	0.89484	293.15	293.15	0	354.21	354.21	0.0805383	0.0805149

534	80.92	11.0854	20.0008	0.0148561	0.891749	293.15	293.15	0	354.038	354.038	0.0804986	0.0804757

535	80.75	11.0954	20.0008	0.0148702	0.888093	293.15	293.15	0	353.872	353.872	0.08046	0.0804364

536	80.58	11.1255	20.0008	0.0149113	0.886083	293.15	293.15	0	353.707	353.707	0.080422	0.0803976

537	80.41	11.1341	20.0091	0.0149236	0.879863	293.15	293.15	0	353.552	353.552	0.080382	0.0803587

538	80.24	11.1161	20.0081	0.0149002	0.875323	293.15	293.15	0	353.381	353.381	0.0803432	0.0803195

539	80.08	11.1437	20.0008	0.0149379	0.87212	293.15	293.15	0	353.205	353.205	0.0803052	0.0802818

540	79.91	11.153	20.0008	0.0149511	0.866442	293.15	293.15	0	353.045	353.045	0.080267	0.0802426

541	79.75	11.0875	19.9987	0.0148641	0.860388	293.15	293.15	0	352.885	352.885	0.080229	0.0802042

542	79.57	11.0173	19.9977	0.0147707	0.859538	293.15	293.15	0	352.711	352.711	0.0801887	0.0801642

543	79.41	11.0455	20.0008	0.0148093	0.853712	293.15	293.15	0	352.547	352.547	0.0801504	0.0801263

544	79.25	11.0912	19.9935	0.0148713	0.848152	293.15	293.15	0	352.379	352.379	0.0801119	0.0800879

545	79.07	11.1567	19.9977	0.0149599	0.844006	293.15	293.15	0	352.208	352.208	0.0800731	0.080048

546	78.91	11.2184	20.0008	0.0150433	0.840887	293.15	293.15	0	352.051	352.051	0.0800339	0.0800097

547	78.74	11.263	20.0008	0.0151039	0.837038	293.15	293.15	0	351.879	351.879	0.0799959	0.0799702

548	78.57	11.3201	19.9946	0.0151812	0.831163	293.15	293.15	0	351.707	351.707	0.079958	0.0799315

549	78.41	11.2655	19.9966	0.0151089	0.824256	293.15	293.15	0	351.542	351.542	0.0799187	0.0798932

550	78.24	11.1712	20.0008	0.0149831	0.822892	293.15	293.15	0	351.386	351.386	0.0798798	0.0798535

551	78.07	11.1061	20.0008	0.0148966	0.820289	293.15	293.15	0	351.222	351.222	0.0798404	0.0798141

552	77.9	11.0813	20.0008	0.0148641	0.817377	293.15	293.15	0	351.048	351.048	0.0798018	0.0797751

553	77.73	11.0886	20.0008	0.0148747	0.810643	293.15	293.15	0	350.884	350.884	0.0797623	0.0797357

554	77.56	11.0843	20.0008	0.0148696	0.807328	293.15	293.15	0	350.711	350.711	0.0797242	0.0796973

555	77.4	11.0604	20.0008	0.0148383	0.80438	293.15	293.15	0	350.538	350.538	0.0796853	0.0796579

556	77.23	11.0707	20.0008	0.0148529	0.798912	293.15	293.15	0	350.383	350.383	0.079647	0.0796195

557	77.06	11.0851	20.0008	0.0148729	0.796434	293.15	293.15	0	350.217	350.217	0.0796066	0.0795795

558	76.89	11.1084	20.0008	0.0149049	0.791406	293.15	293.15	0	350.046	350.046	0.0795685	0.0795404

559	76.73	11.0664	19.9914	0.0148493	0.787246	293.15	293.15	0	349.879	349.879	0.07953	0.0795028

560	76.56	10.9953	19.9946	0.0147547	0.779678	293.15	293.15	0	349.707	349.707	0.0794915	0.0794643

561	76.39	11.0169	20.0008	0.0147844	0.774517	293.15	293.15	0	349.536	349.536	0.079453	0.0794245

562	76.22	11.0194	20.0008	0.0147885	0.772404	293.15	293.15	0	349.379	349.379	0.0794142	0.0793858

563	76.06	10.917	20.0008	0.0146518	0.770671	293.15	293.15	0	349.213	349.213	0.0793749	0.0793466

564	75.89	10.824	20.0008	0.0145277	0.767416	293.15	293.15	0	349.044	349.044	0.0793364	0.0793085

565	75.72	10.8599	19.9925	0.0145766	0.761309	293.15	293.15	0	348.875	348.875	0.0792971	0.0792695

566	75.56	10.9195	19.9904	0.0146573	0.758301	293.15	293.15	0	348.703	348.703	0.0792584	0.0792302

567	75.39	10.9999	19.9904	0.014766	0.75442	293.15	293.15	0	348.555	348.555	0.0792201	0.0791912

568	75.22	11.0337	19.9977	0.0148121	0.751288	293.15	293.15	0	348.387	348.387	0.0791808	0.0791521

569	75.05	11.0797	20.0008	0.0148746	0.744937	293.15	293.15	0	348.217	348.217	0.0791427	0.0791136

570	74.88	11.1718	19.9935	0.0149991	0.740236	293.15	293.15	0	348.04	348.04	0.0791035	0.079074

571	74.72	11.1494	19.9977	0.0149697	0.735069	293.15	293.15	0	347.871	347.871	0.0790649	0.0790355

572	74.55	11.0904	19.9935	0.0148913	0.729975	293.15	293.15	0	347.716	347.716	0.079026	0.0789969

573	74.38	11.11	19.9966	0.0149184	0.72715	293.15	293.15	0	347.55	347.55	0.0789868	0.078957

574	74.22	11.0482	20.0008	0.0148361	0.72283	293.15	293.15	0	347.384	347.384	0.0789481	0.0789185

575	74.05	10.9999	20.0008	0.014772	0.719325	293.15	293.15	0	347.212	347.212	0.0789098	0.0788791

576	73.88	10.9394	19.9946	0.0146915	0.71767	293.15	293.15	0	347.04	347.04	0.0788706	0.0788406

577	73.71	10.8034	19.9966	0.0145095	0.71245	293.15	293.15	0	346.876	346.876	0.0788312	0.0788014

578	73.55	10.6838	20.0008	0.0143497	0.708021	293.15	293.15	0	346.719	346.719	0.0787927	0.0787626

579	73.38	10.7094	20.0008	0.0143848	0.706285	293.15	293.15	0	346.555	346.555	0.0787539	0.0787228

580	73.21	10.8122	20.0008	0.0145236	0.702683	293.15	293.15	0	346.382	346.382	0.0787153	0.0786844

581	73.04	10.8401	20.0008	0.0145618	0.695202	293.15	293.15	0	346.218	346.218	0.0786767	0.0786457

582	72.88	10.8738	19.9956	0.0146078	0.691501	293.15	293.15	0	346.044	346.044	0.078638	0.0786064

583	72.71	10.8795	20.0008	0.0146163	0.6895	293.15	293.15	0	345.88	345.88	0.078599	0.0785674

584	72.54	10.8537	20.0008	0.0145823	0.68707	293.15	293.15	0	345.707	345.707	0.07856	0.0785287

585	72.37	10.8291	19.9966	0.0145499	0.681495	293.15	293.15	0	345.543	345.543	0.0785212	0.0784896

586	72.21	10.7834	19.9904	0.0144893	0.673508	293.15	293.15	0	345.377	345.377	0.0784825	0.0784508

587	72.04	10.7503	19.9987	0.0144456	0.67172	293.15	293.15	0	345.22	345.22	0.0784429	0.078411

588	71.87	10.7357	20.0008	0.0144267	0.668719	293.15	293.15	0	345.051	345.051	0.0784049	0.0783726

589	71.7	10.7814	20.0008	0.0144888	0.663718	293.15	293.15	0	344.884	344.884	0.0783658	0.0783333

590	71.53	10.8452	19.9925	0.0145754	0.660081	293.15	293.15	0	344.705	344.705	0.0783269	0.0782939

591	71.37	10.817	19.9935	0.0145382	0.655833	293.15	293.15	0	344.537	344.537	0.0782888	0.0782559

592	71.2	10.7575	20.0008	0.0144589	0.6522	293.15	293.15	0	344.371	344.371	0.0782496	0.0782164

593	71.04	10.7469	20.0008	0.0144454	0.648237	293.15	293.15	0	344.216	344.216	0.078211	0.0781783

594	70.87	10.7684	20.0008	0.014475	0.642666	293.15	293.15	0	344.048	344.048	0.078172	0.0781386

595	70.7	10.8596	20.0008	0.0145984	0.639326	293.15	293.15	0	343.879	343.879	0.0781331	0.0780992

596	70.53	10.8892	19.9987	0.0146389	0.633581	293.15	293.15	0	343.704	343.704	0.0780937	0.0780595

597	70.36	10.9	19.9904	0.0146542	0.631347	293.15	293.15	0	343.556	343.556	0.0780548	0.0780211

598	70.19	10.899	19.9966	0.0146535	0.629475	293.15	293.15	0	343.385	343.385	0.0780151	0.0779818

599	70.03	10.9194	19.9998	0.0146818	0.62343	293.15	293.15	0	343.211	343.211	0.077977	0.0779426

600	69.86	10.9238	19.9904	0.0146884	0.622979	293.15	293.15	0	343.045	343.045	0.0779375	0.0779031

601	69.69	10.9571	19.9904	0.0147339	0.614261	293.15	293.15	0	342.875	342.875	0.0778991	0.0778647

602	69.53	10.9361	19.9914	0.0147065	0.611939	293.15	293.15	0	342.71	342.71	0.0778603	0.0778261

603	69.36	10.8752	20.0008	0.0146253	0.610124	293.15	293.15	0	342.554	342.554	0.0778215	0.077787

604	69.19	10.794	19.9956	0.0145168	0.60663	293.15	293.15	0	342.38	342.38	0.0777825	0.077748

605	69.02	10.747	19.9956	0.0144544	0.603348	293.15	293.15	0	342.216	342.216	0.0777436	0.0777087

606	68.86	10.7159	20.0008	0.0144132	0.597654	293.15	293.15	0	342.042	342.042	0.0777055	0.07767

607	68.69	10.6507	20.0008	0.0143262	0.592247	293.15	293.15	0	341.879	341.879	0.0776667	0.0776313

608	68.52	10.6211	20.0008	0.0142871	0.588538	293.15	293.15	0	341.713	341.713	0.077628	0.0775922

609	68.36	10.6931	20.0008	0.0143847	0.584864	293.15	293.15	0	341.552	341.552	0.077589	0.0775529

610	68.19	10.7318	19.9966	0.0144375	0.581538	293.15	293.15	0	341.385	341.385	0.077549	0.0775136

611	68.02	10.7913	19.9998	0.0145183	0.577704	293.15	293.15	0	341.212	341.212	0.0775106	0.0774748

612	67.85	10.8194	20.0008	0.0145568	0.574268	293.15	293.15	0	341.04	341.04	0.0774705	0.0774347

613	67.68	10.8206	20.0008	0.0145592	0.571116	293.15	293.15	0	340.875	340.875	0.0774321	0.0773959

614	67.52	10.8346	20.0008	0.0145787	0.564707	293.15	293.15	0	340.709	340.709	0.0773932	0.0773578

615	67.35	10.7608	20.0008	0.0144802	0.561896	293.15	293.15	0	340.549	340.549	0.0773546	0.0773187

616	67.19	10.683	19.9977	0.0143761	0.557752	293.15	293.15	0	340.381	340.381	0.0773167	0.0772804

617	67.02	10.6295	19.9987	0.014305	0.553087	293.15	293.15	0	340.208	340.208	0.0772773	0.0772412

618	66.85	10.6287	20.0008	0.0143046	0.550134	293.15	293.15	0	340.038	340.038	0.0772376	0.0772017

619	66.68	10.6252	20.0008	0.0143006	0.546041	293.15	293.15	0	339.887	339.887	0.0771994	0.0771626

620	66.51	10.691	20.0008	0.0143899	0.544014	293.15	293.15	0	339.713	339.713	0.0771599	0.0771223

621	66.35	10.7722	20.0008	0.0145	0.538736	293.15	293.15	0	339.549	339.549	0.0771219	0.0770849

622	66.18	10.8119	19.9935	0.014554	0.533484	293.15	293.15	0	339.382	339.382	0.0770826	0.0770456

623	66.01	10.7848	19.9977	0.0145184	0.530179	293.15	293.15	0	339.212	339.212	0.0770433	0.077006

624	65.84	10.7488	20.0008	0.0144706	0.525708	293.15	293.15	0	339.039	339.039	0.0770041	0.0769666

625	65.67	10.7464	20.0008	0.0144682	0.521601	293.15	293.15	0	338.871	338.871	0.0769645	0.0769269

626	65.51	10.7234	20.0008	0.0144378	0.518213	293.15	293.15	0	338.719	338.719	0.0769261	0.0768885

627	65.34	10.6526	19.9946	0.0143432	0.515554	293.15	293.15	0	338.545	338.545	0.0768867	0.0768494

628	65.17	10.5863	19.9966	0.0142548	0.512344	293.15	293.15	0	338.378	338.378	0.0768482	0.0768104

629	65.01	10.5367	20.0008	0.0141887	0.505861	293.15	293.15	0	338.208	338.208	0.0768095	0.0767714

630	64.84	10.5257	20.0008	0.0141746	0.504513	293.15	293.15	0	338.041	338.041	0.0767697	0.0767319

631	64.67	10.5508	20.0008	0.0142091	0.50158	293.15	293.15	0	337.887	337.887	0.0767315	0.0766921

632	64.5	10.542	20.0008	0.014198	0.498934	293.15	293.15	0	337.714	337.714	0.0766926	0.0766532

633	64.33	10.5479	20.0008	0.0142066	0.495487	293.15	293.15	0	337.55	337.55	0.0766533	0.0766138

634	64.17	10.5574	20.0008	0.0142202	0.490028	293.15	293.15	0	337.377	337.377	0.0766147	0.0765759

635	64	10.5642	20.0008	0.0142301	0.48699	293.15	293.15	0	337.213	337.213	0.0765756	0.0765367

636	63.83	10.5724	19.9904	0.0142418	0.48294	293.15	293.15	0	337.039	337.039	0.076537	0.0764971

637	63.67	10.6034	19.9946	0.0142842	0.479301	293.15	293.15	0	336.885	336.885	0.0764976	0.0764581

638	63.5	10.6308	20.0008	0.0143219	0.476513	293.15	293.15	0	336.719	336.719	0.076458	0.0764187

639	63.33	10.6179	20.0008	0.0143052	0.47399	293.15	293.15	0	336.555	336.555	0.0764193	0.0763801

640	63.17	10.5749	20.0102	0.014248	0.466941	293.15	293.15	0	336.373	336.373	0.0763812	0.0763416

641	63	10.5755	20.0112	0.0142495	0.458885	293.15	293.15	0	336.208	336.208	0.0763427	0.0763019

642	62.83	10.5747	20.0019	0.0142492	0.459167	293.15	293.15	0	336.044	336.044	0.0763036	0.076263

643	62.66	10.5045	20.0008	0.0141553	0.454689	293.15	293.15	0	335.877	335.877	0.0762631	0.0762229

644	62.49	10.4337	20.0008	0.0140607	0.453031	293.15	293.15	0	335.717	335.717	0.0762245	0.0761837

645	62.33	10.4172	20.0008	0.0140391	0.448048	293.15	293.15	0	335.55	335.55	0.0761856	0.0761446

646	62.16	10.4511	20.0008	0.0140855	0.44286	293.15	293.15	0	335.377	335.377	0.0761473	0.076106

647	61.99	10.4613	19.9925	0.0141	0.440981	293.15	293.15	0	335.207	335.207	0.0761079	0.0760663

648	61.82	10.4782	19.9904	0.0141234	0.439412	293.15	293.15	0	335.04	335.04	0.0760684	0.0760271

649	61.66	10.4631	19.9977	0.0141038	0.434604	293.15	293.15	0	334.883	334.883	0.0760292	0.0759887

650	61.49	10.4841	19.9935	0.0141328	0.429543	293.15	293.15	0	334.714	334.714	0.0759904	0.0759489

651	61.33	10.4829	19.9977	0.0141319	0.424981	293.15	293.15	0	334.546	334.546	0.0759531	0.0759111

652	61.15	10.4461	20.0008	0.0140831	0.424931	293.15	293.15	0	334.378	334.378	0.0759119	0.0758697

653	60.99	10.3685	20.0008	0.0139792	0.42286	293.15	293.15	0	334.216	334.216	0.0758723	0.0758311

654	60.82	10.2682	20.0008	0.0138446	0.415109	293.15	293.15	0	334.042	334.042	0.0758338	0.0757929

655	60.66	10.2059	20.0008	0.0137614	0.41212	293.15	293.15	0	333.878	333.878	0.0757956	0.0757539

656	60.49	10.1864	20.0008	0.0137357	0.40939	293.15	293.15	0	333.712	333.712	0.075757	0.0757148

657	60.32	10.2337	20.0008	0.0138003	0.408218	293.15	293.15	0	333.548	333.548	0.0757171	0.0756753

658	60.15	10.3262	20.0008	0.0139257	0.401563	293.15	293.15	0	333.384	333.384	0.0756781	0.0756367

659	59.99	10.3765	20.0008	0.0139942	0.397471	293.15	293.15	0	333.211	333.211	0.0756401	0.0755974

660	59.82	10.3437	19.9956	0.0139506	0.39612	293.15	293.15	0	333.038	333.038	0.0756008	0.075558

661	59.65	10.3269	20.0008	0.0139287	0.39019	293.15	293.15	0	332.874	332.874	0.0755625	0.0755192

662	59.48	10.2973	19.9904	0.0138894	0.38647	293.15	293.15	0	332.71	332.71	0.0755229	0.0754797

663	59.32	10.2609	19.9946	0.0138411	0.385429	293.15	293.15	0	332.553	332.553	0.0754833	0.0754408

664	59.15	10.2575	20.0008	0.0138372	0.380266	293.15	293.15	0	332.381	332.381	0.0754443	0.0754011

665	58.98	10.2835	20.0008	0.0138729	0.375689	293.15	293.15	0	332.215	332.215	0.0754062	0.0753622

666	58.82	10.3133	20.0008	0.013914	0.371526	293.15	293.15	0	332.043	332.043	0.0753669	0.075323

667	58.65	10.3382	20.0008	0.0139482	0.367012	293.15	293.15	0	331.871	331.871	0.0753275	0.0752834

668	58.47	10.3792	20.0008	0.0140042	0.365025	293.15	293.15	0	331.714	331.714	0.0752883	0.075243

669	58.31	10.3587	20.0008	0.0139773	0.363872	293.15	293.15	0	331.549	331.549	0.0752485	0.0752044

670	58.14	10.3288	20.0008	0.0139377	0.358206	293.15	293.15	0	331.379	331.379	0.0752093	0.0751654

671	57.97	10.3623	20.0091	0.0139836	0.354813	293.15	293.15	0	331.212	331.212	0.0751713	0.075126

672	57.81	10.3777	19.9946	0.014005	0.352567	293.15	293.15	0	331.047	331.047	0.0751312	0.0750866

673	57.64	10.3143	19.9987	0.0139201	0.347925	293.15	293.15	0	330.874	330.874	0.0750924	0.0750476

674	57.48	10.2397	19.9925	0.0138202	0.343431	293.15	293.15	0	330.714	330.714	0.0750539	0.0750093

675	57.32	11.1563	19.9977	0.015058	0.319011	293.15	293.15	0	330.553	330.553	0.0750241	0.0749717

676	57.19	16.0498	20.0008	0.0216638	0.261173	293.15	293.15	0	330.38	330.38	0.0750123	0.0749427

677	57.08	23.2481	20.0008	0.0313811	0.210605	293.15	293.15	0	330.213	330.213	0.0749963	0.0749156

678	56.93	29.8121	20.0008	0.0402431	0.17625	293.15	293.15	0	330.043	330.043	0.074968	0.0748814

679	56.76	35.4777	20.0008	0.0478935	0.146992	293.15	293.15	0	329.87	329.87	0.0749355	0.0748417

680	56.58	40.6336	20.0008	0.0548567	0.122074	293.15	293.15	0	329.71	329.71	0.0749001	0.0748004

681	56.4	45.6072	20.0008	0.0615747	0.0992054	293.15	293.15	0	329.549	329.549	0.0748641	0.0747567

682	56.21	50.4367	20.0008	0.0680989	0.075055	293.15	293.15	0	329.376	329.376	0.0748262	0.0747128

683	56.02	55.3265	20.0008	0.0747054	0.053435	293.15	293.15	0	329.212	329.212	0.0747884	0.0746681

684	55.82	59.9086	20.0008	0.0808972	0.0364017	293.15	293.15	0	329.046	329.046	0.074748	0.0746222

685	55.62	64.3186	20.0008	0.0868575	0.0141542	293.15	293.15	0	328.874	328.874	0.0747086	0.0745754

686	55.43	68.6394	20.0008	0.0926979	0.00350843	293.15	293.15	0	328.707	328.707	0.0746665	0.0745291

687	55.23	72.7841	20.0008	0.0983014	-0.0111092	293.15	293.15	0	328.553	328.553	0.0746246	0.0744823

688	55.04	76.4003	20.0008	0.103191	-0.0285838	293.15	293.15	0	328.371	328.371	0.0745846	0.0744388

689	54.87	79.3768	20.0008	0.107217	-0.0467593	293.15	293.15	0	328.208	328.208	0.0745462	0.0743974

690	54.69	81.7221	20.0008	0.110391	-0.0678231	293.15	293.15	0	328.042	328.042	0.0745064	0.0743564

691	54.52	83.4285	20.0008	0.112702	-0.0885523	293.15	293.15	0	327.886	327.886	0.0744691	0.0743173

692	54.36	84.7176	20.0008	0.114449	-0.107529	293.15	293.15	0	327.714	327.714	0.0744309	0.0742784

693	54.19	85.5554	20.0008	0.115586	-0.127451	293.15	293.15	0	327.549	327.549	0.0743913	0.0742398

694	54.04	86.039	19.9966	0.116245	-0.153857	293.15	293.15	0	327.369	327.369	0.0743542	0.0742028

695	53.88	86.2837	19.9998	0.116582	-0.174235	293.15	293.15	0	327.202	327.202	0.0743157	0.0741649

696	53.71	86.2387	19.9914	0.116527	-0.191703	293.15	293.15	0	327.047	327.047	0.0742771	0.0741268

697	53.55	85.8489	19.9987	0.116006	-0.209534	293.15	293.15	0	326.882	326.882	0.0742379	0.0740877

698	53.38	85.1682	20.0008	0.115092	-0.230783	293.15	293.15	0	326.713	326.713	0.0741975	0.0740498

699	53.22	84.2033	20.0091	0.113793	-0.245463	293.15	293.15	0	326.545	326.545	0.0741567	0.0740105

700	53.05	82.9591	20.0029	0.112118	-0.258281	293.15	293.15	0	326.372	326.372	0.0741149	0.0739713

701	52.88	81.4852	20.0008	0.110132	-0.268598	293.15	293.15	0	326.22	326.22	0.0740721	0.0739304

702	52.7	79.794	20.0008	0.107852	-0.279815	293.15	293.15	0	326.05	326.05	0.0740277	0.0738888

703	52.52	77.9502	20.0008	0.105365	-0.280203	293.15	293.15	0	325.878	325.878	0.0739811	0.0738458

704	52.33	75.8792	20.0008	0.102572	-0.279225	293.15	293.15	0	325.71	325.71	0.0739336	0.0738022

705	52.13	73.5929	20.0008	0.0994872	-0.274113	293.15	293.15	0	325.54	325.54	0.0738845	0.0737561

706	51.93	71.041	19.9935	0.0960432	-0.267087	293.15	293.15	0	325.372	325.372	0.0738324	0.0737081

707	51.72	68.1668	19.9966	0.0921633	-0.244962	293.15	293.15	0	325.202	325.202	0.0737792	0.073659

708	51.49	64.7637	20.0008	0.0875684	-0.214147	293.15	293.15	0	325.044	325.044	0.0737199	0.0736053

709	51.25	60.8647	20.0008	0.0823024	-0.176608	293.15	293.15	0	324.89	324.89	0.0736584	0.0735496

710	51.01	56.4581	20.0008	0.0763494	-0.116886	293.15	293.15	0	324.708	324.708	0.0735925	0.073491

711	50.74	51.8292	20.0008	0.0700953	-0.0574737	293.15	293.15	0	324.543	324.543	0.0735243	0.0734293

712	50.46	46.9928	20.0008	0.0635599	0.0134236	293.15	293.15	0	324.379	324.379	0.0734513	0.0733627

713	50.18	42.4131	20.0008	0.0573705	0.0913731	293.15	293.15	0	324.205	324.205	0.0733808	0.0732977

714	49.94	37.9531	20.0008	0.0513414	0.152067	293.15	293.15	0	324.04	324.04	0.0733194	0.0732406

715	49.75	33.519	20.0008	0.0453456	0.199044	293.15	293.15	0	323.876	323.876	0.0732685	0.0731968

716	49.61	29.0373	20.0008	0.0392844	0.232934	293.15	293.15	0	323.714	323.714	0.0732273	0.0731623

717	49.48	24.6687	20.0008	0.0333755	0.254058	293.15	293.15	0	323.555	323.555	0.0731924	0.0731328

718	49.37	20.7951	20.0008	0.0281355	0.265831	293.15	293.15	0	323.382	323.382	0.0731649	0.0731077

719	49.28	17.372	19.9977	0.0235048	0.269216	293.15	293.15	0	323.218	323.218	0.0731382	0.0730851

720	49.19	14.4709	19.9987	0.0195802	0.268388	293.15	293.15	0	323.049	323.049	0.0731146	0.0730641

721	49.09	12.1997	20.0008	0.0165075	0.263004	293.15	293.15	0	322.871	322.871	0.0730916	0.073042

722	48.99	10.4328	20.0008	0.0141171	0.256063	293.15	293.15	0	322.711	322.711	0.0730672	0.0730184

723	48.89	9.14385	19.9935	0.0123734	0.247866	293.15	293.15	0	322.551	322.551	0.0730425	0.0729942

724	48.79	8.24922	19.9977	0.0111631	0.234712	293.15	293.15	0	322.377	322.377	0.0730175	0.0729697

725	48.67	7.6435	20.0008	0.0103438	0.226431	293.15	293.15	0	322.214	322.214	0.0729904	0.0729422

726	48.55	7.33667	20.0008	0.00992895	0.216951	293.15	293.15	0	322.045	322.045	0.0729614	0.0729129

727	48.42	7.31827	20.0008	0.00990443	0.204221	293.15	293.15	0	321.884	321.884	0.0729326	0.0728831

728	48.28	7.39555	20.0008	0.0100094	0.195246	293.15	293.15	0	321.717	321.717	0.0729017	0.0728514

729	48.15	7.58954	20.0008	0.0102724	0.187307	293.15	293.15	0	321.546	321.546	0.07287	0.0728191

730	48	7.81442	20.0008	0.0105772	0.180401	293.15	293.15	0	321.373	321.373	0.0728361	0.0727853

731	47.86	8.01499	20.0008	0.0108492	0.170639	293.15	293.15	0	321.207	321.207	0.0728023	0.0727512

732	47.7	8.16175	19.9946	0.0110484	0.166141	293.15	293.15	0	321.045	321.045	0.0727663	0.0727149

733	47.55	8.36431	19.9956	0.0113231	0.16068	293.15	293.15	0	320.889	320.889	0.072731	0.0726785

734	47.39	8.58541	20.0008	0.011623	0.157809	293.15	293.15	0	320.716	320.716	0.0726943	0.072642

735	47.23	8.80572	20.0008	0.0119218	0.149057	293.15	293.15	0	320.542	320.542	0.072657	0.0726044

736	47.08	8.97702	19.9904	0.0121543	0.142235	293.15	293.15	0	320.369	320.369	0.0726205	0.072568

737	46.92	9.13672	19.9904	0.0123711	0.139456	293.15	293.15	0	320.205	320.205	0.0725827	0.0725293

738	46.75	9.31655	19.9946	0.0126153	0.13469	293.15	293.15	0	320.038	320.038	0.0725446	0.0724902

739	46.59	9.453	19.9914	0.0128007	0.133115	293.15	293.15	0	319.884	319.884	0.0725058	0.0724517

740	46.42	9.59812	19.9998	0.0129978	0.125552	293.15	293.15	0	319.712	319.712	0.0724672	0.0724128

741	46.26	9.68607	20.0008	0.0131176	0.119687	293.15	293.15	0	319.545	319.545	0.0724292	0.0723749

742	46.09	9.74731	20.0008	0.0132012	0.117214	293.15	293.15	0	319.373	319.373	0.0723895	0.0723356

743	45.92	9.77951	20.0008	0.0132455	0.111358	293.15	293.15	0	319.202	319.202	0.0723505	0.0722958

744	45.76	9.79487	20.0008	0.0132669	0.110496	293.15	293.15	0	319.045	319.045	0.0723116	0.0722568

745	45.59	9.81882	19.9925	0.0133001	0.109693	293.15	293.15	0	318.88	318.88	0.0722715	0.0722172

746	45.42	9.85385	19.9987	0.0133482	0.106317	293.15	293.15	0	318.71	318.71	0.0722335	0.0721783

747	45.26	9.86379	20.0008	0.0133623	0.0996078	293.15	293.15	0	318.542	318.542	0.0721942	0.072139

748	45.09	9.85959	20.0008	0.0133573	0.0979342	293.15	293.15	0	318.369	318.369	0.0721551	0.0720993

749	44.92	9.84093	20.0008	0.0133327	0.0957191	293.15	293.15	0	318.221	318.221	0.072116	0.072059

750	44.75	9.83479	20.0008	0.0133251	0.0945401	293.15	293.15	0	318.054	318.054	0.0720751	0.0720192

751	44.58	9.82632	20.0008	0.0133143	0.0895265	293.15	293.15	0	317.884	317.884	0.0720362	0.0719794

752	44.41	9.82966	19.9977	0.0133195	0.0878808	293.15	293.15	0	317.711	317.711	0.0719966	0.07194

753	44.25	9.88013	20.0112	0.0133886	0.0832524	293.15	293.15	0	317.543	317.543	0.0719579	0.0719014

754	44.08	9.92577	20.0039	0.0134511	0.0776851	293.15	293.15	0	317.383	317.383	0.0719187	0.0718623

755	43.91	9.95231	19.9998	0.0134878	0.0774644	293.15	293.15	0	317.217	317.217	0.0718788	0.0718219

756	43.75	9.95848	19.9904	0.0134968	0.0736176	293.15	293.15	0	317.051	317.051	0.0718401	0.0717828

757	43.58	10.021	19.9966	0.0135823	0.0707882	293.15	293.15	0	316.879	316.879	0.071801	0.0717434

758	43.41	10.0642	20.0008	0.0136415	0.0693494	293.15	293.15	0	316.707	316.707	0.0717612	0.071704

759	43.25	10.0325	20.0008	0.0135992	0.0638457	293.15	293.15	0	316.559	316.559	0.0717219	0.0716651

760	43.07	9.93291	20.0008	0.0134649	0.0638215	293.15	293.15	0	316.386	316.386	0.0716817	0.0716245

761	42.91	9.90388	20.0008	0.0134262	0.0615535	293.15	293.15	0	316.213	316.213	0.0716429	0.0715854

762	42.74	9.86945	20.0112	0.0133803	0.0587857	293.15	293.15	0	316.048	316.048	0.0716039	0.0715457

763	42.57	9.83333	20.006	0.013332	0.0554868	293.15	293.15	0	315.875	315.875	0.0715648	0.0715063

764	42.4	9.87781	20.0008	0.013393	0.0521537	293.15	293.15	0	315.702	315.702	0.0715245	0.0714662

765	42.23	9.94362	19.9914	0.0134829	0.0509545	293.15	293.15	0	315.554	315.554	0.0714855	0.0714264

766	42.07	9.97794	19.9946	0.0135301	0.0476553	293.15	293.15	0	315.381	315.381	0.0714461	0.0713871

767	41.9	9.94127	20.0008	0.0134811	0.0458006	293.15	293.15	0	315.217	315.217	0.0714066	0.0713479

768	41.73	9.90708	20.0008	0.0134354	0.0406377	293.15	293.15	0	315.046	315.046	0.0713672	0.0713078

769	41.57	9.93724	20.0008	0.013477	0.0373165	293.15	293.15	0	314.87	314.87	0.0713281	0.071269

770	41.4	9.92578	20.0008	0.0134621	0.0383687	293.15	293.15	0	314.708	314.708	0.0712874	0.0712289

771	41.23	9.8655	19.9925	0.0133811	0.0348397	293.15	293.15	0	314.55	314.55	0.0712473	0.071189

772	41.06	9.79843	19.9935	0.0132908	0.0298064	293.15	293.15	0	314.386	314.386	0.0712094	0.07115

773	40.89	9.80961	20.0008	0.0133066	0.029432	293.15	293.15	0	314.213	314.213	0.0711697	0.0711096

774	40.72	9.86207	19.9987	0.0133785	0.0287982	293.15	293.15	0	314.041	314.041	0.0711302	0.0710699

775	40.56	9.89041	19.9904	0.0134176	0.0227942	293.15	293.15	0	313.879	313.879	0.0710906	0.0710306

776	40.39	9.88387	19.9904	0.0134094	0.0210278	293.15	293.15	0	313.709	313.709	0.0710508	0.0709908

777	40.22	9.85036	19.9977	0.0133646	0.0220236	293.15	293.15	0	313.537	313.537	0.0710105	0.0709507

778	40.05	9.83052	20.0008	0.0133384	0.0198463	293.15	293.15	0	313.378	313.378	0.0709705	0.0709107

779	39.88	9.80267	20.0008	0.0133013	0.0204377	293.15	293.15	0	313.215	313.215	0.0709314	0.070871

780	39.71	9.77057	20.0008	0.0132584	0.0167292	293.15	293.15	0	313.043	313.043	0.0708918	0.0708316

781	39.55	9.77715	20.0008	0.013268	0.013088	293.15	293.15	0	312.878	312.878	0.0708533	0.0707931

782	39.38	9.76924	19.9946	0.013258	0.00999071	293.15	293.15	0	312.711	312.711	0.070814	0.0707534

783	39.21	9.75966	19.9956	0.0132456	0.00606606	293.15	293.15	0	312.541	312.541	0.0707752	0.070714

784	39.06	9.77708	19.9904	0.0132699	0.000135396	293.15	293.15	0	312.374	312.374	0.0707373	0.0706765

785	38.9	9.73694	19.9956	0.0132161	-0.00320642	293.15	293.15	0	312.22	312.22	0.0706992	0.0706387

786	38.74	9.5817	20.0008	0.013006	-0.00879507	293.15	293.15	0	312.047	312.047	0.070662	0.0706018

787	38.58	9.47116	20.0008	0.0128565	-0.0172606	293.15	293.15	0	311.873	311.873	0.0706254	0.070565

788	38.43	9.33794	20.0008	0.0126763	-0.0282011	293.15	293.15	0	311.71	311.71	0.070589	0.0705297

789	38.29	9.21004	20.0008	0.0125032	-0.0400633	293.15	293.15	0	311.537	311.537	0.070554	0.0704945

790	38.14	9.10734	20.0008	0.0123644	-0.0539738	293.15	293.15	0	311.372	311.372	0.0705186	0.0704591

791	37.99	8.97368	19.9966	0.0121835	-0.0679013	293.15	293.15	0	311.216	311.216	0.0704845	0.0704244

792	37.84	8.85901	19.9904	0.0120283	-0.0875872	293.15	293.15	0	311.043	311.043	0.0704505	0.0703904

793	37.71	8.71895	19.9904	0.0118386	-0.108011	293.15	293.15	0	310.879	310.879	0.070418	0.070358

794	37.56	8.54161	19.9904	0.0115984	-0.128306	293.15	293.15	0	310.706	310.706	0.0703839	0.0703241

795	37.42	8.43739	19.9998	0.0114573	-0.150081	293.15	293.15	0	310.541	310.541	0.0703514	0.0702913

796	37.28	8.32301	20.0008	0.0113025	-0.17677	293.15	293.15	0	310.375	310.375	0.0703189	0.0702581

797	37.15	8.16979	20.0008	0.0110949	-0.20077	293.15	293.15	0	310.215	310.215	0.0702864	0.0702266

798	37.02	7.99304	20.0008	0.0108552	-0.231024	293.15	293.15	0	310.047	310.047	0.070256	0.0701963

799	36.89	7.86443	20.0008	0.010681	-0.265351	293.15	293.15	0	309.874	309.874	0.0702258	0.0701658

800	36.76	7.73543	20.0008	0.0105062	-0.300654	293.15	293.15	0	309.705	309.705	0.0701955	0.0701353

801	36.64	7.60492	20.0008	0.0103294	-0.333212	293.15	293.15	0	309.554	309.554	0.0701652	0.0701055

802	36.51	7.4449	20.0008	0.0101124	-0.374042	293.15	293.15	0	309.381	309.381	0.0701352	0.0700759

803	36.39	7.34464	20.0008	0.0099766	-0.417665	293.15	293.15	0	309.216	309.216	0.0701064	0.0700466

804	36.27	7.2717	20.0008	0.00987789	-0.462618	293.15	293.15	0	309.049	309.049	0.0700782	0.0700174

805	36.15	7.17606	20.0008	0.00974832	-0.510646	293.15	293.15	0	308.879	308.879	0.0700496	0.0699896

806	36.03	7.07638	20.0008	0.00961326	-0.562514	293.15	293.15	0	308.711	308.711	0.0700218	0.0699616

807	35.91	6.98784	20.0008	0.00949331	-0.612383	293.15	293.15	0	308.549	308.549	0.0699936	0.0699335

808	35.8	6.93595	19.9998	0.00942316	-0.671953	293.15	293.15	0	308.375	308.375	0.0699661	0.0699065

809	35.68	6.84729	19.9904	0.00930302	-0.730532	293.15	293.15	0	308.211	308.211	0.0699393	0.06988

810	35.57	6.71875	19.9966	0.00912869	-0.79208	293.15	293.15	0	308.046	308.046	0.0699131	0.0698539

811	35.46	6.60363	20.0008	0.00897258	-0.861025	293.15	293.15	0	307.875	307.875	0.0698865	0.0698274

812	35.35	6.48691	20.0008	0.00881428	-0.930006	293.15	293.15	0	307.708	307.708	0.0698612	0.069802

813	35.25	6.39782	19.9956	0.00869351	-0.995766	293.15	293.15	0	307.554	307.554	0.0698357	0.0697762

814	35.14	6.28607	20.0008	0.00854194	-1.07348	293.15	293.15	0	307.381	307.381	0.0698111	0.0697517

815	35.04	6.09211	20.0112	0.00827864	-1.14948	293.15	293.15	0	307.216	307.216	0.0697856	0.069727

816	34.94	5.91801	20.006	0.0080423	-1.2377	293.15	293.15	0	307.042	307.042	0.0697613	0.0697031

817	34.84	5.79005	20.0008	0.00786864	-1.3224	293.15	293.15	0	306.879	306.879	0.0697377	0.0696792

818	34.74	5.67188	20.0008	0.00770829	-1.41209	293.15	293.15	0	306.713	306.713	0.0697148	0.0696562

819	34.64	5.58257	20.0008	0.00758714	-1.50442	293.15	293.15	0	306.551	306.551	0.0696921	0.0696333

820	34.54	5.48885	20.0008	0.00745998	-1.6013	293.15	293.15	0	306.385	306.385	0.0696691	0.0696099

821	34.45	5.3893	19.9914	0.00732489	-1.70642	293.15	293.15	0	306.212	306.212	0.0696464	0.0695878

822	34.35	5.27158	19.9904	0.00716511	-1.81512	293.15	293.15	0	306.04	306.04	0.0696246	0.0695654

823	34.26	5.2222	19.9998	0.00709819	-1.92242	293.15	293.15	0	305.874	305.874	0.069602	0.0695434

824	34.17	5.18147	20.0008	0.00704302	-2.03576	293.15	293.15	0	305.709	305.709	0.06958	0.0695215

825	34.08	5.09186	20.0008	0.00692141	-2.14424	293.15	293.15	0	305.554	305.554	0.0695589	0.0694999

826	33.99	4.96105	20.0008	0.00674378	-2.26657	293.15	293.15	0	305.384	305.384	0.0695379	0.0694792

827	33.91	4.85315	20.0008	0.00659728	-2.3993	293.15	293.15	0	305.207	305.207	0.0695172	0.069459

828	33.81	4.7467	20.0008	0.00645275	-2.52276	293.15	293.15	0	305.047	305.047	0.0694965	0.0694375

829	33.73	4.74232	20.0008	0.00644696	-2.6578	293.15	293.15	0	304.878	304.878	0.069476	0.0694173

830	33.65	4.79876	20.0008	0.00652386	-2.79751	293.15	293.15	0	304.71	304.71	0.0694566	0.0693976

831	33.56	4.7999	20.0008	0.00652557	-2.9422	293.15	293.15	0	304.54	304.54	0.0694376	0.0693784

832	33.48	4.67411	20.0008	0.00635471	-3.08806	293.15	293.15	0	304.375	304.375	0.0694177	0.069359

833	33.4	4.51602	20.0008	0.00613993	-3.2281	293.15	293.15	0	304.219	304.219	0.0693987	0.0693401

834	33.32	4.40241	19.9946	0.00598561	-3.38092	293.15	293.15	0	304.054	304.054	0.0693796	0.0693212

835	33.24	4.30877	19.9966	0.00585844	-3.54524	293.15	293.15	0	303.881	303.881	0.069361	0.0693025

836	33.17	4.16722	19.9956	0.00566612	-3.70566	293.15	293.15	0	303.716	303.716	0.0693428	0.069285

837	33.09	4.07151	20.0008	0.00553611	-3.87251	293.15	293.15	0	303.552	303.552	0.0693245	0.0692658

838	33.01	4.01958	19.9956	0.00546562	-4.0521	293.15	293.15	0	303.379	303.379	0.069307	0.0692479

839	32.94	3.98472	20.0008	0.00541834	-4.2263	293.15	293.15	0	303.215	303.215	0.0692894	0.0692309
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RT54-0.2 GNP 3.txt
# Name: RT54-0.2 GNP 3

# Date: Tue May 21 11:11:16 2024

# Weight: 10 mg

Time(s)	Temperature(°C)	Heat flow(mW)	Gas 1(sccm/min)	DSC_RAW(µV)	POWER(%)	TEMP_CJR_FURNACE(K)	TEMP_CJR_SAMPLE(K)	TEMP_FURNACE(K)	TEMP_NOM_FURNACE(K)	TEMP_NOM_SAMPLE(K)	VOLTAGE_REFERENCE(V)	VOLTAGE_SAMPLE(V)

0	29.89	-0.074005	20.0008	-0.000100724	0.0798077	293.15	293.15	0	303.264	303.264	0.0685516	0.068508

1	29.92	-0.22152	20.0008	-0.000301497	0.141917	293.15	293.15	0	303.433	303.433	0.0685566	0.068514

2	30	-0.760237	20.0008	-0.00103468	0.188943	293.15	293.15	0	303.601	303.601	0.0685738	0.0685341

3	30.13	-2.00916	20.0008	-0.00273436	0.222958	293.15	293.15	0	303.774	303.774	0.0686009	0.068565

4	30.28	-3.70444	20.0008	-0.00504132	0.248302	293.15	293.15	0	303.944	303.944	0.0686339	0.0686008

5	30.45	-5.53586	20.0008	-0.00753328	0.265376	293.15	293.15	0	304.112	304.112	0.0686726	0.0686419

6	30.64	-7.27421	19.9987	-0.0098983	0.274401	293.15	293.15	0	304.277	304.277	0.0687138	0.0686847

7	30.83	-8.89414	19.9925	-0.0121019	0.284623	293.15	293.15	0	304.432	304.432	0.0687581	0.0687306

8	31.02	-10.2345	20.0008	-0.0139249	0.288378	293.15	293.15	0	304.599	304.599	0.0688016	0.0687756

9	31.22	-11.3323	20.0008	-0.0154176	0.288951	293.15	293.15	0	304.769	304.769	0.0688479	0.0688238

10	31.42	-12.1471	19.9987	-0.016525	0.289631	293.15	293.15	0	304.942	304.942	0.068894	0.0688695

11	31.6	-12.7251	19.9925	-0.0173104	0.294099	293.15	293.15	0	305.111	305.111	0.0689387	0.0689144

12	31.79	-13.0793	20.0008	-0.0177912	0.293893	293.15	293.15	0	305.271	305.271	0.0689821	0.0689586

13	31.98	-13.2875	19.9998	-0.0180734	0.293723	293.15	293.15	0	305.437	305.437	0.0690265	0.0690034

14	32.17	-13.4145	19.9904	-0.0182451	0.298935	293.15	293.15	0	305.602	305.602	0.0690698	0.0690476

15	32.35	-13.491	19.9914	-0.0183481	0.298296	293.15	293.15	0	305.774	305.774	0.0691143	0.0690919

16	32.53	-13.5106	20.0008	-0.0183737	0.298824	293.15	293.15	0	305.938	305.938	0.0691562	0.0691336

17	32.71	-13.4607	20.0008	-0.0183048	0.300094	293.15	293.15	0	306.111	306.111	0.0691989	0.0691768

18	32.88	-13.3936	20.0008	-0.0182127	0.301882	293.15	293.15	0	306.269	306.269	0.06924	0.0692173

19	33.06	-13.3513	20.0008	-0.0181542	0.304532	293.15	293.15	0	306.432	306.432	0.0692817	0.0692598

20	33.23	-13.3116	19.9956	-0.0180992	0.307784	293.15	293.15	0	306.605	306.605	0.0693218	0.0693001

21	33.41	-13.2708	20.0008	-0.0180428	0.307472	293.15	293.15	0	306.769	306.769	0.0693634	0.0693416

22	33.58	-13.2344	20.0008	-0.0179924	0.308814	293.15	293.15	0	306.942	306.942	0.069405	0.0693829

23	33.75	-13.1327	20.0008	-0.0178532	0.313652	293.15	293.15	0	307.106	307.106	0.0694445	0.0694224

24	33.92	-12.994	20.0008	-0.0176637	0.314062	293.15	293.15	0	307.279	307.279	0.0694854	0.0694633

25	34.09	-12.9103	19.9914	-0.017549	0.316061	293.15	293.15	0	307.427	307.427	0.0695247	0.0695027

26	34.26	-12.9059	19.9956	-0.0175422	0.316767	293.15	293.15	0	307.6	307.6	0.0695646	0.0695436

27	34.43	-12.8897	19.9904	-0.0175192	0.324	293.15	293.15	0	307.771	307.771	0.069605	0.0695835

28	34.6	-12.8343	19.9998	-0.017443	0.325165	293.15	293.15	0	307.938	307.938	0.0696438	0.0696234

29	34.77	-12.8001	20.0008	-0.0173956	0.327423	293.15	293.15	0	308.111	308.111	0.0696839	0.0696629

30	34.94	-12.7673	20.0008	-0.0173502	0.331197	293.15	293.15	0	308.282	308.282	0.0697239	0.0697029

31	35.1	-12.7208	20.0008	-0.0172861	0.334006	293.15	293.15	0	308.432	308.432	0.0697631	0.0697421

32	35.27	-12.795	20.0008	-0.017386	0.337344	293.15	293.15	0	308.604	308.604	0.069803	0.0697823

33	35.44	-12.8575	20.0008	-0.0174701	0.340529	293.15	293.15	0	308.77	308.77	0.0698418	0.0698216

34	35.6	-12.8529	20.0008	-0.0174629	0.345989	293.15	293.15	0	308.938	308.938	0.0698813	0.069861

35	35.78	-12.8319	20.0008	-0.0174335	0.346816	293.15	293.15	0	309.106	309.106	0.0699218	0.0699018

36	35.94	-12.8316	20.0008	-0.0174323	0.351391	293.15	293.15	0	309.279	309.279	0.0699609	0.069941

37	36.11	-12.8812	20.0008	-0.0174987	0.354299	293.15	293.15	0	309.427	309.427	0.07	0.0699807

38	36.27	-12.903	20.0008	-0.0175275	0.358618	293.15	293.15	0	309.595	309.595	0.0700386	0.0700191

39	36.44	-12.9035	20.0008	-0.0175272	0.362598	293.15	293.15	0	309.764	309.764	0.0700783	0.0700586

40	36.61	-12.8985	20.0008	-0.0175195	0.365304	293.15	293.15	0	309.942	309.942	0.0701177	0.070098

41	36.77	-12.9098	20.0008	-0.0175339	0.367869	293.15	293.15	0	310.103	310.103	0.0701568	0.0701374

42	36.94	-12.9311	20.0008	-0.0175621	0.368555	293.15	293.15	0	310.269	310.269	0.0701977	0.0701779

43	37.11	-12.989	20.0008	-0.0176398	0.374118	293.15	293.15	0	310.44	310.44	0.0702364	0.0702168

44	37.28	-13.0317	19.9998	-0.0176968	0.376928	293.15	293.15	0	310.613	310.613	0.0702757	0.0702564

45	37.45	-13.0542	19.9904	-0.0177264	0.379358	293.15	293.15	0	310.762	310.762	0.0703151	0.0702961

46	37.61	-13.0421	19.9904	-0.0177092	0.382526	293.15	293.15	0	310.935	310.935	0.0703539	0.0703355

47	37.78	-13.017	20.0008	-0.0176742	0.388167	293.15	293.15	0	311.099	311.099	0.0703938	0.0703755

48	37.95	-12.9919	20.0008	-0.0176391	0.390427	293.15	293.15	0	311.272	311.272	0.0704334	0.0704152

49	38.12	-13.0234	20.0008	-0.0176811	0.392524	293.15	293.15	0	311.444	311.444	0.0704727	0.070455

50	38.28	-13.0159	20.0008	-0.01767	0.395428	293.15	293.15	0	311.609	311.609	0.0705114	0.070494

51	38.45	-13.0441	20.0008	-0.0177073	0.401499	293.15	293.15	0	311.766	311.766	0.0705505	0.0705334

52	38.62	-13.107	20.0008	-0.0177918	0.403063	293.15	293.15	0	311.939	311.939	0.0705904	0.0705733

53	38.78	-13.1732	20.0008	-0.0178807	0.40502	293.15	293.15	0	312.103	312.103	0.0706292	0.0706119

54	38.95	-13.2264	20.0008	-0.017952	0.407625	293.15	293.15	0	312.274	312.274	0.070669	0.070652

55	39.12	-13.2839	20.0008	-0.0180292	0.415446	293.15	293.15	0	312.449	312.449	0.0707082	0.0706912

56	39.29	-13.3301	20.0008	-0.018091	0.41695	293.15	293.15	0	312.611	312.611	0.0707476	0.0707309

57	39.45	-13.3821	20.0008	-0.0181606	0.420323	293.15	293.15	0	312.77	312.77	0.0707866	0.0707699

58	39.62	-13.3814	20.0008	-0.0181588	0.426325	293.15	293.15	0	312.943	312.943	0.0708256	0.070809

59	39.79	-13.3866	20.0008	-0.0181649	0.429108	293.15	293.15	0	313.107	313.107	0.0708652	0.070849

60	39.96	-13.3926	20.0008	-0.0181721	0.430624	293.15	293.15	0	313.277	313.277	0.0709054	0.0708893

61	40.12	-13.3691	20.0008	-0.0181392	0.433449	293.15	293.15	0	313.445	313.445	0.0709449	0.0709282

62	40.29	-13.3798	20.0008	-0.0181529	0.436365	293.15	293.15	0	313.601	313.601	0.0709834	0.0709683

63	40.45	-13.3894	20.0008	-0.018165	0.444221	293.15	293.15	0	313.765	313.765	0.0710216	0.0710063

64	40.63	-13.4102	20.0008	-0.0181923	0.444374	293.15	293.15	0	313.933	313.933	0.0710624	0.0710477

65	40.79	-13.4152	20.0008	-0.0181981	0.446031	293.15	293.15	0	314.103	314.103	0.071102	0.071087

66	40.96	-13.3836	20.0008	-0.0181543	0.449733	293.15	293.15	0	314.279	314.279	0.0711411	0.0711263

67	41.13	-13.3785	20.0008	-0.0181465	0.453611	293.15	293.15	0	314.432	314.432	0.0711808	0.0711659

68	41.29	-13.3955	20.0019	-0.0181686	0.456648	293.15	293.15	0	314.597	314.597	0.0712194	0.071205

69	41.47	-13.4363	20.0102	-0.0182229	0.458548	293.15	293.15	0	314.77	314.77	0.0712591	0.0712451

70	41.63	-13.5481	20.0008	-0.0183737	0.463701	293.15	293.15	0	314.937	314.937	0.0712981	0.0712845

71	41.8	-13.6064	20.0008	-0.0184518	0.470233	293.15	293.15	0	315.108	315.108	0.0713371	0.0713233

72	41.96	-13.6441	20.0008	-0.018502	0.473614	293.15	293.15	0	315.273	315.273	0.0713762	0.0713621

73	42.13	-13.6744	20.0008	-0.0185421	0.474245	293.15	293.15	0	315.428	315.428	0.0714159	0.0714018

74	42.3	-13.734	20.0008	-0.018622	0.475362	293.15	293.15	0	315.601	315.601	0.0714552	0.0714419

75	42.47	-13.7662	19.9904	-0.0186647	0.482404	293.15	293.15	0	315.765	315.765	0.0714944	0.071481

76	42.63	-13.7007	20.0008	-0.0185749	0.484635	293.15	293.15	0	315.938	315.938	0.0715335	0.0715199

77	42.8	-13.6759	20.0008	-0.0185404	0.488898	293.15	293.15	0	316.103	316.103	0.0715728	0.0715599

78	42.97	-13.7403	19.9904	-0.0186268	0.492359	293.15	293.15	0	316.275	316.275	0.0716121	0.0715992

79	43.13	-13.7957	19.9998	-0.018701	0.495563	293.15	293.15	0	316.43	316.43	0.0716511	0.0716387

80	43.3	-13.8087	20.0008	-0.0187176	0.499509	293.15	293.15	0	316.596	316.596	0.07169	0.0716779

81	43.47	-13.8173	20.0008	-0.0187283	0.499671	293.15	293.15	0	316.77	316.77	0.07173	0.071718

82	43.64	-13.8273	20.0008	-0.0187409	0.504808	293.15	293.15	0	316.941	316.941	0.0717694	0.0717569

83	43.8	-13.8512	20.0008	-0.0187723	0.509297	293.15	293.15	0	317.106	317.106	0.0718084	0.0717959

84	43.97	-13.9094	20.0008	-0.0188502	0.51364	293.15	293.15	0	317.28	317.28	0.0718473	0.0718366

85	44.14	-13.9433	19.9966	-0.0188952	0.516437	293.15	293.15	0	317.444	317.444	0.0718866	0.0718753

86	44.31	-14.028	19.9904	-0.019009	0.519965	293.15	293.15	0	317.606	317.606	0.0719262	0.0719153

87	44.48	-13.9966	19.9987	-0.0189655	0.5214	293.15	293.15	0	317.765	317.765	0.0719665	0.0719549

88	44.64	-13.948	20.0008	-0.0188988	0.526956	293.15	293.15	0	317.939	317.939	0.0720043	0.0719927

89	44.81	-13.9508	20.0008	-0.0189015	0.529869	293.15	293.15	0	318.109	318.109	0.0720441	0.0720331

90	44.97	-13.9059	19.9956	-0.0188397	0.533817	293.15	293.15	0	318.276	318.276	0.0720828	0.0720723

91	45.14	-13.8815	20.0008	-0.0188058	0.540499	293.15	293.15	0	318.432	318.432	0.0721214	0.0721109

92	45.31	-13.9161	20.0008	-0.0188517	0.542089	293.15	293.15	0	318.6	318.6	0.0721617	0.0721512

93	45.47	-13.9874	20.0008	-0.0189473	0.54384	293.15	293.15	0	318.769	318.769	0.0722002	0.0721899

94	45.64	-14.033	20.0008	-0.0190081	0.548523	293.15	293.15	0	318.933	318.933	0.0722396	0.07223

95	45.81	-14.0984	20.0008	-0.0190957	0.554643	293.15	293.15	0	319.106	319.106	0.0722783	0.0722694

96	45.98	-14.1757	20.0008	-0.0191994	0.555326	293.15	293.15	0	319.274	319.274	0.072318	0.072309

97	46.15	-14.2746	20.0008	-0.0193324	0.555552	293.15	293.15	0	319.444	319.444	0.0723586	0.0723495

98	46.31	-14.3157	20.0008	-0.019387	0.563229	293.15	293.15	0	319.61	319.61	0.0723969	0.0723875

99	46.48	-14.2883	20.0008	-0.0193489	0.564645	293.15	293.15	0	319.767	319.767	0.0724366	0.0724271

100	46.65	-14.2878	19.9998	-0.0193473	0.567837	293.15	293.15	0	319.938	319.938	0.0724757	0.0724666

101	46.81	-14.2444	19.9956	-0.0192875	0.570751	293.15	293.15	0	320.095	320.095	0.072515	0.0725055

102	46.98	-14.2371	20.0008	-0.0192766	0.575734	293.15	293.15	0	320.277	320.277	0.0725535	0.0725451

103	47.15	-14.2284	19.9904	-0.0192639	0.583431	293.15	293.15	0	320.442	320.442	0.0725919	0.0725839

104	47.32	-14.297	20.0008	-0.0193559	0.58608	293.15	293.15	0	320.607	320.607	0.0726317	0.0726238

105	47.48	-14.4298	20.0008	-0.0195347	0.588033	293.15	293.15	0	320.762	320.762	0.0726698	0.0726628

106	47.65	-14.5831	19.9914	-0.0197411	0.589899	293.15	293.15	0	320.933	320.933	0.0727103	0.0727032

107	47.82	-14.6463	19.9946	-0.0198257	0.595743	293.15	293.15	0	321.1	321.1	0.0727496	0.072742

108	47.99	-14.6427	20.0008	-0.0198198	0.601053	293.15	293.15	0	321.28	321.28	0.072788	0.0727813

109	48.16	-14.589	20.0008	-0.0197461	0.600918	293.15	293.15	0	321.445	321.445	0.0728279	0.0728212

110	48.33	-14.5276	20.0008	-0.019662	0.601824	293.15	293.15	0	321.6	321.6	0.0728677	0.0728612

111	48.49	-14.5492	20.0008	-0.0196902	0.606515	293.15	293.15	0	321.766	321.766	0.0729067	0.0729002

112	48.66	-14.6007	20.0008	-0.0197589	0.612712	293.15	293.15	0	321.935	321.935	0.0729455	0.0729392

113	48.83	-14.6105	20.0039	-0.0197712	0.618261	293.15	293.15	0	322.113	322.113	0.0729845	0.0729789

114	48.99	-14.5858	20.0091	-0.0197368	0.620738	293.15	293.15	0	322.273	322.273	0.0730232	0.0730178

115	49.16	-14.5312	20.0008	-0.0196618	0.623731	293.15	293.15	0	322.433	322.433	0.0730629	0.0730574

116	49.33	-14.5007	20.0008	-0.0196196	0.62804	293.15	293.15	0	322.607	322.607	0.0731024	0.0730969

117	49.5	-14.4978	20.0008	-0.0196147	0.630679	293.15	293.15	0	322.771	322.771	0.0731417	0.0731369

118	49.66	-14.531	19.9987	-0.0196586	0.633296	293.15	293.15	0	322.939	322.939	0.0731807	0.0731755

119	49.83	-14.5734	19.9925	-0.0197149	0.639929	293.15	293.15	0	323.108	323.108	0.07322	0.0732149

120	50	-14.5922	20.0008	-0.0197394	0.643	293.15	293.15	0	323.276	323.276	0.073259	0.0732542

121	50.16	-14.6021	19.9998	-0.0197518	0.646235	293.15	293.15	0	323.438	323.438	0.0732979	0.0732929

122	50.33	-14.6376	19.9914	-0.0197988	0.648227	293.15	293.15	0	323.602	323.602	0.0733367	0.0733321

123	50.49	-14.6574	20.0008	-0.0198246	0.65435	293.15	293.15	0	323.776	323.776	0.0733759	0.0733706

124	50.66	-14.6901	20.0008	-0.0198678	0.659018	293.15	293.15	0	323.941	323.941	0.073415	0.0734108

125	50.83	-14.6972	20.0008	-0.0198763	0.661778	293.15	293.15	0	324.096	324.096	0.0734544	0.0734505

126	51	-14.6965	20.0008	-0.0198744	0.664129	293.15	293.15	0	324.269	324.269	0.0734936	0.0734894

127	51.17	-14.7411	20.0008	-0.0199338	0.670008	293.15	293.15	0	324.433	324.433	0.0735327	0.0735296

128	51.33	-14.8273	20.0008	-0.0200493	0.673552	293.15	293.15	0	324.616	324.616	0.0735714	0.073568

129	51.5	-14.8944	20.0008	-0.020139	0.675012	293.15	293.15	0	324.779	324.779	0.0736111	0.0736077

130	51.67	-14.9891	20.0008	-0.020266	0.67945	293.15	293.15	0	324.945	324.945	0.0736504	0.0736472

131	51.84	-15.0236	20.0008	-0.0203117	0.681087	293.15	293.15	0	325.1	325.1	0.073689	0.0736862

132	52	-14.9519	20.0008	-0.0202137	0.688032	293.15	293.15	0	325.273	325.273	0.0737279	0.0737249

133	52.17	-14.9218	20.0008	-0.0201719	0.689371	293.15	293.15	0	325.437	325.437	0.0737673	0.0737648

134	52.34	-14.9866	20.0008	-0.0202585	0.691571	293.15	293.15	0	325.61	325.61	0.0738073	0.0738049

135	52.51	-15.1139	20.0008	-0.0204295	0.696317	293.15	293.15	0	325.764	325.764	0.0738459	0.0738437

136	52.67	-15.1932	19.9977	-0.0205357	0.702867	293.15	293.15	0	325.932	325.932	0.0738848	0.073883

137	52.84	-15.2736	19.9935	-0.0206434	0.708197	293.15	293.15	0	326.105	326.105	0.0739234	0.0739218

138	53	-15.3607	19.9977	-0.0207601	0.712277	293.15	293.15	0	326.276	326.276	0.0739614	0.0739594

139	53.18	-15.3992	19.9904	-0.0208109	0.71364	293.15	293.15	0	326.442	326.442	0.0740028	0.0740009

140	53.34	-15.3682	19.9925	-0.020768	0.719424	293.15	293.15	0	326.608	326.608	0.0740416	0.0740395

141	53.51	-15.2895	20.0008	-0.0206607	0.723913	293.15	293.15	0	326.766	326.766	0.0740792	0.0740784

142	53.67	-15.3057	20.0008	-0.0206814	0.725672	293.15	293.15	0	326.936	326.936	0.0741186	0.0741179

143	53.84	-15.3707	20.0008	-0.0207683	0.73078	293.15	293.15	0	327.1	327.1	0.0741571	0.0741566

144	54.01	-15.4166	20.0008	-0.0208292	0.737431	293.15	293.15	0	327.273	327.273	0.0741958	0.0741956

145	54.18	-15.4654	20.0008	-0.0208941	0.737581	293.15	293.15	0	327.441	327.441	0.0742361	0.0742356

146	54.34	-15.5329	20.0019	-0.0209842	0.739145	293.15	293.15	0	327.601	327.601	0.0742753	0.0742749

147	54.52	-15.6501	20.0102	-0.0211414	0.745987	293.15	293.15	0	327.767	327.767	0.074315	0.0743154

148	54.68	-15.6976	20.0008	-0.0212045	0.749811	293.15	293.15	0	327.933	327.933	0.0743527	0.0743539

149	54.85	-15.7383	20.0008	-0.0212584	0.75343	293.15	293.15	0	328.104	328.104	0.0743923	0.0743936

150	55.02	-15.7593	20.0008	-0.0212857	0.756502	293.15	293.15	0	328.278	328.278	0.0744321	0.0744332

151	55.18	-15.7765	20.0008	-0.0213079	0.7618	293.15	293.15	0	328.441	328.441	0.0744711	0.0744715

152	55.35	-15.7379	20.0008	-0.0212547	0.764845	293.15	293.15	0	328.608	328.608	0.07451	0.0745105

153	55.51	-15.7426	20.0008	-0.0212599	0.770493	293.15	293.15	0	328.763	328.763	0.0745476	0.074549

154	55.68	-15.833	20.0008	-0.0213809	0.771864	293.15	293.15	0	328.936	328.936	0.0745879	0.0745888

155	55.85	-15.9972	20.0008	-0.0216015	0.78194	293.15	293.15	0	329.1	329.1	0.0746258	0.0746282

156	56.02	-16.1501	20.0008	-0.0218069	0.785659	293.15	293.15	0	329.273	329.273	0.0746643	0.0746677

157	56.19	-16.2895	20.0008	-0.0219941	0.787303	293.15	293.15	0	329.446	329.446	0.0747038	0.0747071

158	56.35	-16.4417	20.0008	-0.0221984	0.788565	293.15	293.15	0	329.601	329.601	0.0747433	0.0747459

159	56.52	-16.5566	20.0008	-0.0223524	0.792545	293.15	293.15	0	329.767	329.767	0.0747822	0.074786

160	56.69	-16.7093	20.0008	-0.0225574	0.800783	293.15	293.15	0	329.939	329.939	0.0748195	0.0748248

161	56.86	-16.9183	20.0008	-0.0228384	0.805551	293.15	293.15	0	330.104	330.104	0.0748586	0.0748638

162	57.02	-17.1504	20.0008	-0.0231505	0.811036	293.15	293.15	0	330.277	330.277	0.0748978	0.0749031

163	57.19	-17.4086	20.0008	-0.0234979	0.81845	293.15	293.15	0	330.44	330.44	0.0749353	0.0749413

164	57.35	-17.7612	20.0008	-0.0239726	0.826065	293.15	293.15	0	330.613	330.613	0.0749733	0.0749807

165	57.52	-18.2332	19.9977	-0.0246084	0.8309	293.15	293.15	0	330.781	330.781	0.0750127	0.0750203

166	57.69	-18.7938	19.9925	-0.0253637	0.834737	293.15	293.15	0	330.946	330.946	0.0750509	0.0750591

167	57.86	-19.3587	19.9987	-0.0261248	0.841143	293.15	293.15	0	331.101	331.101	0.0750889	0.0750987

168	58.02	-19.979	19.9904	-0.0269606	0.853174	293.15	293.15	0	331.269	331.269	0.0751256	0.0751369

169	58.19	-20.7352	19.9925	-0.0279795	0.861369	293.15	293.15	0	331.448	331.448	0.0751631	0.0751771

170	58.36	-21.7034	20.0008	-0.0292846	0.869538	293.15	293.15	0	331.607	331.607	0.0752003	0.0752157

171	58.52	-22.9251	20.0008	-0.0309315	0.880925	293.15	293.15	0	331.769	331.769	0.0752366	0.0752547

172	58.69	-24.4679	20.0008	-0.0330113	0.89366	293.15	293.15	0	331.932	331.932	0.075273	0.0752936

173	58.85	-26.2773	20.0071	-0.0354508	0.909261	293.15	293.15	0	332.106	332.106	0.0753075	0.0753315

174	59.02	-28.4158	20.0102	-0.038334	0.926888	293.15	293.15	0	332.272	332.272	0.0753421	0.0753699

175	59.18	-30.8753	20.0008	-0.0416499	0.94643	293.15	293.15	0	332.444	332.444	0.0753763	0.0754083

176	59.34	-33.7305	20.0008	-0.0454992	0.966994	293.15	293.15	0	332.609	332.609	0.0754093	0.0754464

177	59.51	-37.0314	20.0008	-0.0499494	0.988405	293.15	293.15	0	332.765	332.765	0.075443	0.0754848

178	59.67	-40.6801	20.0008	-0.0548682	1.01344	293.15	293.15	0	332.937	332.937	0.075474	0.0755226

179	59.84	-44.7093	20.0008	-0.0602996	1.04045	293.15	293.15	0	333.101	333.101	0.075506	0.0755619

180	60	-48.9941	20.0008	-0.0660752	1.06968	293.15	293.15	0	333.274	333.274	0.0755387	0.075601

181	60.18	-53.5219	20.0008	-0.0721778	1.09098	293.15	293.15	0	333.438	333.438	0.0755739	0.075642

182	60.36	-57.8635	20.0008	-0.0780285	1.11145	293.15	293.15	0	333.604	333.604	0.0756105	0.0756838

183	60.54	-62.0593	20.0008	-0.0836817	1.1304	293.15	293.15	0	333.766	333.766	0.075648	0.0757268

184	60.72	-65.9116	20.0008	-0.0888714	1.15014	293.15	293.15	0	333.932	333.932	0.0756865	0.0757695

185	60.91	-69.3343	20.0008	-0.093481	1.16789	293.15	293.15	0	334.105	334.105	0.0757265	0.0758137

186	61.11	-72.4077	20.0008	-0.097619	1.17812	293.15	293.15	0	334.277	334.277	0.0757689	0.0758592

187	61.3	-75.0776	20.0008	-0.101213	1.18711	293.15	293.15	0	334.443	334.443	0.0758119	0.075905

188	61.5	-77.2983	20.0008	-0.1042	1.19364	293.15	293.15	0	334.609	334.609	0.0758552	0.0759505

189	61.69	-79.1319	20.0008	-0.106666	1.19965	293.15	293.15	0	334.764	334.764	0.0758998	0.0759969

190	61.89	-80.5108	20.0008	-0.108518	1.20641	293.15	293.15	0	334.934	334.934	0.075944	0.0760424

191	62.08	-81.554	20.0008	-0.109917	1.20627	293.15	293.15	0	335.11	335.11	0.0759901	0.0760882

192	62.28	-82.2562	20.0008	-0.110857	1.20777	293.15	293.15	0	335.28	335.28	0.0760355	0.0761331

193	62.47	-82.6722	20.0008	-0.111411	1.20928	293.15	293.15	0	335.431	335.431	0.0760792	0.0761778

194	62.66	-82.8433	20.0008	-0.111635	1.20633	293.15	293.15	0	335.604	335.604	0.0761252	0.0762234

195	62.85	-82.7011	20.0008	-0.111438	1.20243	293.15	293.15	0	335.768	335.768	0.0761693	0.0762662

196	63.04	-82.2689	19.9956	-0.110849	1.20451	293.15	293.15	0	335.936	335.936	0.0762136	0.0763106

197	63.23	-81.6574	20.0008	-0.110019	1.19835	293.15	293.15	0	336.106	336.106	0.0762586	0.0763549

198	63.4	-80.9307	19.9935	-0.109034	1.19303	293.15	293.15	0	336.279	336.279	0.0763022	0.0763969

199	63.59	-80.0124	19.9904	-0.107791	1.19041	293.15	293.15	0	336.446	336.446	0.0763459	0.0764393

200	63.76	-78.9595	19.9914	-0.106367	1.18885	293.15	293.15	0	336.599	336.599	0.076388	0.0764796

201	63.93	-77.6579	19.9946	-0.104608	1.18455	293.15	293.15	0	336.773	336.773	0.0764308	0.0765199

202	64.11	-76.073	19.9914	-0.102467	1.17606	293.15	293.15	0	336.938	336.938	0.0764747	0.0765622

203	64.28	-74.5106	20.0008	-0.100358	1.17171	293.15	293.15	0	337.11	337.11	0.0765175	0.0766014

204	64.45	-72.8912	20.0008	-0.0981715	1.16963	293.15	293.15	0	337.283	337.283	0.076559	0.0766407

205	64.61	-71.2155	20.0008	-0.0959099	1.16702	293.15	293.15	0	337.431	337.431	0.0765991	0.0766792

206	64.78	-69.3715	20.0008	-0.0934215	1.15734	293.15	293.15	0	337.605	337.605	0.076642	0.0767194

207	64.95	-67.3457	20.0008	-0.0906889	1.15103	293.15	293.15	0	337.768	337.768	0.0766836	0.0767584

208	65.12	-65.1731	20.0008	-0.0877589	1.14646	293.15	293.15	0	337.941	337.941	0.0767252	0.076797

209	65.28	-62.8358	20.0008	-0.0846073	1.134	293.15	293.15	0	338.105	338.105	0.0767682	0.0768357

210	65.45	-60.5955	20.0008	-0.0815867	1.13342	293.15	293.15	0	338.271	338.271	0.076807	0.0768737

211	65.6	-58.6318	20.0008	-0.0789391	1.1253	293.15	293.15	0	338.433	338.433	0.076847	0.0769104

212	65.77	-55.9019	20.0008	-0.0752599	1.11215	293.15	293.15	0	338.599	338.599	0.0768924	0.0769493

213	65.94	-52.2125	19.9966	-0.0702892	1.09112	293.15	293.15	0	338.772	338.772	0.0769389	0.0769892

214	66.12	-47.7859	19.9904	-0.0643267	1.06584	293.15	293.15	0	338.944	338.944	0.0769878	0.0770302

215	66.29	-42.9659	20.0039	-0.0578353	1.04171	293.15	293.15	0	339.11	339.11	0.0770349	0.0770699

216	66.45	-38.0548	20.0081	-0.0512221	1.02653	293.15	293.15	0	339.275	339.275	0.0770794	0.0771078

217	66.61	-33.1629	20.0008	-0.0446353	1.01069	293.15	293.15	0	339.43	339.43	0.0771222	0.0771449

218	66.75	-28.8042	20.0039	-0.0387671	0.998824	293.15	293.15	0	339.6	339.6	0.0771611	0.0771788

219	66.9	-24.955	20.0081	-0.0335851	0.992901	293.15	293.15	0	339.769	339.769	0.0771978	0.0772128

220	67.04	-21.9812	20.0008	-0.0295816	0.991993	293.15	293.15	0	339.941	339.941	0.0772318	0.0772451

221	67.17	-19.5745	20.0008	-0.0263417	0.993437	293.15	293.15	0	340.111	340.111	0.0772647	0.0772766

222	67.31	-17.7279	20.0008	-0.0238558	0.994274	293.15	293.15	0	340.28	340.28	0.0772978	0.0773081

223	67.44	-16.3436	20.0008	-0.0219921	1.00037	293.15	293.15	0	340.438	340.438	0.0773292	0.0773391

224	67.57	-15.3218	20.0008	-0.0206163	1.01112	293.15	293.15	0	340.608	340.608	0.0773602	0.07737

225	67.71	-14.6784	20.0008	-0.0197497	1.01672	293.15	293.15	0	340.765	340.765	0.0773921	0.0774021

226	67.85	-14.2574	20.0008	-0.0191824	1.02328	293.15	293.15	0	340.931	340.931	0.0774259	0.0774355

227	67.99	-14.0167	19.9998	-0.0188578	1.03118	293.15	293.15	0	341.102	341.102	0.0774587	0.0774684

228	68.14	-13.915	19.9914	-0.0187201	1.03983	293.15	293.15	0	341.278	341.278	0.0774929	0.0775027

229	68.29	-13.9049	20.0008	-0.0187056	1.04946	293.15	293.15	0	341.432	341.432	0.077528	0.0775385

230	68.44	-13.904	20.0008	-0.0187036	1.05783	293.15	293.15	0	341.605	341.605	0.0775622	0.0775736

231	68.59	-13.9323	19.9904	-0.0187409	1.06518	293.15	293.15	0	341.771	341.771	0.0775972	0.0776086

232	68.76	-14.0472	20.0008	-0.0188944	1.07268	293.15	293.15	0	341.942	341.942	0.0776345	0.0776462

233	68.91	-14.2592	20.0008	-0.0191787	1.07858	293.15	293.15	0	342.115	342.115	0.0776706	0.0776832

234	69.08	-14.4798	19.9904	-0.0194745	1.08307	293.15	293.15	0	342.271	342.271	0.0777084	0.0777213

235	69.24	-14.6741	19.9946	-0.0197348	1.08663	293.15	293.15	0	342.437	342.437	0.077746	0.0777587

236	69.4	-14.778	20.0008	-0.0198736	1.09216	293.15	293.15	0	342.609	342.609	0.0777842	0.0777972

237	69.57	-14.8527	19.9956	-0.019973	1.10125	293.15	293.15	0	342.774	342.774	0.0778218	0.0778352

238	69.73	-14.922	20.0008	-0.0200653	1.10469	293.15	293.15	0	342.947	342.947	0.0778595	0.0778727

239	69.9	-15.0395	20.0008	-0.0202222	1.10727	293.15	293.15	0	343.095	343.095	0.0778986	0.0779129

240	70.07	-15.125	20.0008	-0.0203362	1.11279	293.15	293.15	0	343.264	343.264	0.0779373	0.0779517

241	70.23	-15.1919	19.9977	-0.0204251	1.12094	293.15	293.15	0	343.441	343.441	0.0779755	0.0779904

242	70.39	-15.286	19.9904	-0.0205505	1.12715	293.15	293.15	0	343.605	343.605	0.0780134	0.0780283

243	70.56	-15.328	19.9904	-0.020606	1.13159	293.15	293.15	0	343.776	343.776	0.0780518	0.0780672

244	70.73	-15.3857	19.9935	-0.0206825	1.13208	293.15	293.15	0	343.942	343.942	0.078092	0.0781072

245	70.9	-15.4606	20.0008	-0.0207821	1.13942	293.15	293.15	0	344.099	344.099	0.0781305	0.0781456

246	71.07	-15.4599	20.0008	-0.0207802	1.14366	293.15	293.15	0	344.267	344.267	0.0781689	0.0781852

247	71.24	-15.4862	20.0008	-0.0208144	1.14535	293.15	293.15	0	344.436	344.436	0.0782089	0.0782254

248	71.4	-15.5249	20.0008	-0.0208654	1.15111	293.15	293.15	0	344.6	344.6	0.0782472	0.0782634

249	71.57	-15.5584	20.0008	-0.0209094	1.15715	293.15	293.15	0	344.774	344.774	0.0782858	0.0783023

250	71.74	-15.6217	19.9987	-0.0209933	1.15987	293.15	293.15	0	344.941	344.941	0.0783251	0.0783411

251	71.9	-15.6289	19.9977	-0.021002	1.16329	293.15	293.15	0	345.111	345.111	0.078363	0.0783793

252	72.07	-15.5636	20.0008	-0.0209132	1.16846	293.15	293.15	0	345.276	345.276	0.078403	0.0784193

253	72.24	-15.498	19.9998	-0.020824	1.17187	293.15	293.15	0	345.431	345.431	0.0784414	0.0784574

254	72.41	-15.4564	19.9966	-0.0207671	1.1757	293.15	293.15	0	345.597	345.597	0.0784807	0.0784973

255	72.57	-15.458	19.9998	-0.0207681	1.1812	293.15	293.15	0	345.768	345.768	0.0785191	0.078536

256	72.74	-15.474	19.9914	-0.0207886	1.18681	293.15	293.15	0	345.944	345.944	0.0785578	0.0785747

257	72.91	-15.4927	20.0008	-0.0208127	1.19188	293.15	293.15	0	346.099	346.099	0.0785964	0.0786137

258	73.07	-15.5631	20.0008	-0.0209062	1.19498	293.15	293.15	0	346.273	346.273	0.0786354	0.0786528

259	73.24	-15.5935	20.0008	-0.020946	1.19655	293.15	293.15	0	346.436	346.436	0.0786752	0.0786922

260	73.41	-15.5071	19.9956	-0.0208289	1.20613	293.15	293.15	0	346.609	346.609	0.0787132	0.0787301

261	73.58	-15.437	19.9904	-0.0207337	1.20921	293.15	293.15	0	346.773	346.773	0.0787518	0.0787697

262	73.75	-15.4589	19.9966	-0.020762	1.21082	293.15	293.15	0	346.937	346.937	0.0787914	0.0788092

263	73.92	-15.4657	19.9904	-0.02077	1.21509	293.15	293.15	0	347.103	347.103	0.0788295	0.0788485

264	74.08	-15.4457	19.9904	-0.0207422	1.21768	293.15	293.15	0	347.275	347.275	0.0788684	0.0788873

265	74.25	-15.4376	19.9998	-0.0207303	1.2249	293.15	293.15	0	347.441	347.441	0.0789076	0.078926

266	74.42	-15.4646	20.0008	-0.0207655	1.22772	293.15	293.15	0	347.604	347.604	0.0789464	0.0789653

267	74.58	-15.4833	20.0008	-0.0207895	1.23313	293.15	293.15	0	347.778	347.778	0.0789852	0.0790039

268	74.74	-15.5117	20.0008	-0.0208267	1.23736	293.15	293.15	0	347.939	347.939	0.0790231	0.0790415

269	74.92	-15.5441	19.9977	-0.020869	1.242	293.15	293.15	0	348.098	348.098	0.0790624	0.0790815

270	75.08	-15.6224	19.9904	-0.0209731	1.24788	293.15	293.15	0	348.271	348.271	0.0791004	0.0791196

271	75.25	-15.6627	19.9935	-0.0210261	1.25224	293.15	293.15	0	348.436	348.436	0.0791389	0.0791594

272	75.42	-15.685	20.0008	-0.0210551	1.25712	293.15	293.15	0	348.605	348.605	0.0791786	0.0791982

273	75.58	-15.6633	20.0008	-0.0210249	1.26305	293.15	293.15	0	348.773	348.773	0.0792164	0.0792366

274	75.75	-15.6307	20.0008	-0.0209801	1.26649	293.15	293.15	0	348.942	348.942	0.0792555	0.0792753

275	75.92	-15.6275	20.0008	-0.0209747	1.26806	293.15	293.15	0	349.103	349.103	0.079295	0.0793151

276	76.09	-15.5984	20.0008	-0.0209346	1.27314	293.15	293.15	0	349.276	349.276	0.0793337	0.0793536

277	76.25	-15.6381	20.0008	-0.0209868	1.27859	293.15	293.15	0	349.44	349.44	0.0793726	0.0793924

278	76.42	-15.682	20.0008	-0.0210447	1.28329	293.15	293.15	0	349.607	349.607	0.0794106	0.0794316

279	76.59	-15.6787	20.0008	-0.0210392	1.28579	293.15	293.15	0	349.761	349.761	0.0794496	0.0794707

280	76.76	-15.6622	20.0008	-0.021016	1.29045	293.15	293.15	0	349.934	349.934	0.0794888	0.0795094

281	76.92	-15.6281	20.0008	-0.0209691	1.2961	293.15	293.15	0	350.099	350.099	0.079527	0.0795478

282	77.09	-15.5821	20.0008	-0.0209063	1.29913	293.15	293.15	0	350.272	350.272	0.0795666	0.0795871

283	77.25	-15.5114	20.0019	-0.0208105	1.30764	293.15	293.15	0	350.444	350.444	0.0796036	0.0796245

284	77.42	-15.5163	20.0102	-0.020816	1.30928	293.15	293.15	0	350.61	350.61	0.0796432	0.0796639

285	77.59	-15.6253	20.0008	-0.0209612	1.31716	293.15	293.15	0	350.774	350.774	0.0796813	0.0797027

286	77.76	-15.6976	20.0008	-0.0210571	1.32082	293.15	293.15	0	350.939	350.939	0.0797205	0.0797419

287	77.92	-15.7096	20.0008	-0.0210722	1.3252	293.15	293.15	0	351.112	351.112	0.0797582	0.0797805

288	78.09	-15.6596	20.0008	-0.0210039	1.32759	293.15	293.15	0	351.275	351.275	0.0797978	0.0798198

289	78.26	-15.686	20.0008	-0.0210383	1.33384	293.15	293.15	0	351.433	351.433	0.0798362	0.0798583

290	78.43	-15.6894	20.0008	-0.0210418	1.33563	293.15	293.15	0	351.606	351.606	0.079876	0.0798975

291	78.59	-15.6759	20.0008	-0.0210227	1.33979	293.15	293.15	0	351.77	351.77	0.0799146	0.0799367

292	78.76	-15.6815	20.0008	-0.0210291	1.34254	293.15	293.15	0	351.941	351.941	0.0799539	0.079976

293	78.93	-15.6323	20.0008	-0.0209621	1.35103	293.15	293.15	0	352.107	352.107	0.0799916	0.080014

294	79.09	-15.5708	19.9977	-0.0208786	1.35637	293.15	293.15	0	352.278	352.278	0.0800296	0.0800522

295	79.26	-15.5804	19.9904	-0.0208904	1.36331	293.15	293.15	0	352.438	352.438	0.0800682	0.0800913

296	79.43	-15.6261	19.9987	-0.0209506	1.36669	293.15	293.15	0	352.61	352.61	0.0801073	0.0801301

297	79.6	-15.6718	20.0008	-0.0210109	1.37206	293.15	293.15	0	352.779	352.779	0.0801463	0.0801702

298	79.76	-15.7116	20.0008	-0.0210632	1.37632	293.15	293.15	0	352.939	352.939	0.0801846	0.0802078

299	79.93	-15.7186	20.0008	-0.0210714	1.37998	293.15	293.15	0	353.104	353.104	0.0802229	0.0802463

300	80.09	-15.7287	20.0008	-0.021084	1.3839	293.15	293.15	0	353.268	353.268	0.080261	0.0802848

301	80.26	-15.6727	20.0008	-0.0210078	1.39138	293.15	293.15	0	353.436	353.436	0.0803005	0.0803244

302	80.43	-15.6225	20.0008	-0.0209395	1.39418	293.15	293.15	0	353.606	353.606	0.0803398	0.0803638

303	80.6	-15.6109	20.0008	-0.0209229	1.39779	293.15	293.15	0	353.778	353.778	0.0803777	0.0804024

304	80.77	-15.5822	20.0008	-0.0208833	1.3997	293.15	293.15	0	353.937	353.937	0.0804173	0.0804419

305	80.93	-15.6222	20.0008	-0.020936	1.40559	293.15	293.15	0	354.099	354.099	0.0804562	0.0804799

306	81.1	-15.6783	20.0008	-0.0210101	1.41276	293.15	293.15	0	354.272	354.272	0.0804939	0.0805193

307	81.27	-15.6968	20.0008	-0.0210337	1.41539	293.15	293.15	0	354.436	354.436	0.080533	0.0805582

308	81.44	-15.7602	20.0008	-0.0211176	1.42031	293.15	293.15	0	354.602	354.602	0.080572	0.0805965

309	81.6	-15.8219	20.0008	-0.0211993	1.42678	293.15	293.15	0	354.774	354.774	0.0806101	0.0806354

310	81.77	-15.8589	20.0008	-0.0212478	1.43292	293.15	293.15	0	354.939	354.939	0.0806485	0.0806741

311	81.94	-15.8735	20.0008	-0.0212663	1.43417	293.15	293.15	0	355.095	355.095	0.080688	0.0807135

312	82.11	-15.9132	20.0008	-0.0213183	1.4369	293.15	293.15	0	355.268	355.268	0.080727	0.080753

313	82.28	-15.9116	19.9956	-0.0213151	1.44387	293.15	293.15	0	355.432	355.432	0.080765	0.0807915

314	82.44	-15.8521	19.9904	-0.0212344	1.44879	293.15	293.15	0	355.605	355.605	0.0808035	0.0808302

315	82.61	-15.7438	19.9956	-0.0210883	1.45477	293.15	293.15	0	355.771	355.771	0.0808414	0.0808677

316	82.78	-15.7486	19.9904	-0.0210936	1.46268	293.15	293.15	0	355.942	355.942	0.08088	0.0809074

317	82.94	-15.8615	19.9904	-0.0212437	1.46548	293.15	293.15	0	356.106	356.106	0.0809188	0.0809459

318	83.11	-15.8787	19.9998	-0.0212658	1.4682	293.15	293.15	0	356.261	356.261	0.0809572	0.0809836

319	83.28	-15.8994	20.0008	-0.0212924	1.47164	293.15	293.15	0	356.436	356.436	0.0809962	0.0810238

320	83.45	-15.9292	20.0008	-0.0213312	1.47457	293.15	293.15	0	356.608	356.608	0.0810346	0.0810625

321	83.61	-15.9464	20.0008	-0.0213531	1.48269	293.15	293.15	0	356.773	356.773	0.0810738	0.0811016

322	83.78	-15.9168	20.0008	-0.0213124	1.48836	293.15	293.15	0	356.947	356.947	0.0811119	0.0811399

323	83.95	-15.8967	20.0008	-0.0212845	1.49188	293.15	293.15	0	357.094	357.094	0.08115	0.0811784

324	84.12	-15.9431	20.0008	-0.0213455	1.49421	293.15	293.15	0	357.265	357.265	0.08119	0.0812186

325	84.28	-15.9772	20.0008	-0.0213902	1.50147	293.15	293.15	0	357.432	357.432	0.081228	0.0812569

326	84.45	-15.9433	20.0008	-0.0213436	1.50526	293.15	293.15	0	357.605	357.605	0.081267	0.0812961

327	84.62	-15.9217	20.0008	-0.0213136	1.50929	293.15	293.15	0	357.775	357.775	0.0813062	0.0813348

328	84.78	-15.8868	20.0008	-0.0212659	1.51578	293.15	293.15	0	357.942	357.942	0.0813444	0.0813721

329	84.95	-15.8909	20.0008	-0.0212703	1.52028	293.15	293.15	0	358.098	358.098	0.0813832	0.0814113

330	85.12	-15.8669	20.0029	-0.0212371	1.52454	293.15	293.15	0	358.266	358.266	0.0814216	0.0814502

331	85.28	-15.7635	20.0071	-0.0210977	1.5281	293.15	293.15	0	358.436	358.436	0.0814603	0.0814885

332	85.45	-15.7301	19.9977	-0.0210519	1.53335	293.15	293.15	0	358.609	358.609	0.0814984	0.0815271

333	85.62	-15.7335	20.0008	-0.0210554	1.5401	293.15	293.15	0	358.773	358.773	0.0815369	0.0815663

334	85.78	-15.7518	20.0008	-0.0210788	1.54448	293.15	293.15	0	358.941	358.941	0.081575	0.0816047

335	85.96	-15.8068	20.0008	-0.0211514	1.5483	293.15	293.15	0	359.094	359.094	0.0816131	0.0816441

336	86.12	-15.8037	20.0008	-0.0211462	1.5521	293.15	293.15	0	359.267	359.267	0.0816526	0.0816827

337	86.29	-15.8457	20.0008	-0.0212013	1.55959	293.15	293.15	0	359.433	359.433	0.0816906	0.0817211

338	86.46	-15.885	20.0008	-0.0212528	1.56221	293.15	293.15	0	359.605	359.605	0.0817303	0.0817605

339	86.63	-15.8501	20.0008	-0.021205	1.56616	293.15	293.15	0	359.769	359.769	0.0817696	0.0817996

340	86.79	-15.8307	20.0008	-0.021178	1.57501	293.15	293.15	0	359.934	359.934	0.0818062	0.0818369

341	86.95	-15.7983	20.0008	-0.0211336	1.57646	293.15	293.15	0	360.099	360.099	0.0818455	0.0818752

342	87.13	-15.7493	20.0008	-0.021067	1.58094	293.15	293.15	0	360.271	360.271	0.0818844	0.0819152

343	87.29	-15.7144	20.0008	-0.0210193	1.5861	293.15	293.15	0	360.445	360.445	0.0819231	0.081953

344	87.46	-15.7028	20.0008	-0.0210027	1.59009	293.15	293.15	0	360.602	360.602	0.0819611	0.0819917

345	87.62	-15.6556	20.0008	-0.0209385	1.59426	293.15	293.15	0	360.775	360.775	0.0820009	0.0820304

346	87.79	-15.6491	19.9914	-0.0209288	1.60276	293.15	293.15	0	360.946	360.946	0.0820378	0.0820684

347	87.95	-15.6333	19.9935	-0.0209067	1.60711	293.15	293.15	0	361.095	361.095	0.0820761	0.082107

348	88.12	-15.649	20.0008	-0.0209266	1.61269	293.15	293.15	0	361.275	361.275	0.0821157	0.082146

349	88.29	-15.6926	20.0008	-0.0209838	1.61676	293.15	293.15	0	361.442	361.442	0.0821531	0.0821853

350	88.46	-15.7088	19.9977	-0.0210044	1.62322	293.15	293.15	0	361.607	361.607	0.0821917	0.082223

351	88.63	-15.7739	19.9987	-0.0210903	1.62801	293.15	293.15	0	361.779	361.779	0.0822308	0.0822627

352	88.79	-15.7811	19.9987	-0.0210989	1.63224	293.15	293.15	0	361.94	361.94	0.082269	0.0823006

353	88.96	-15.7695	19.9925	-0.0210825	1.63799	293.15	293.15	0	362.1	362.1	0.0823072	0.0823393

354	89.13	-15.7897	20.0008	-0.0211083	1.64453	293.15	293.15	0	362.273	362.273	0.0823457	0.0823792

355	89.3	-15.8351	20.0008	-0.0211679	1.64767	293.15	293.15	0	362.438	362.438	0.0823845	0.0824181

356	89.46	-15.8943	20.0008	-0.021246	1.65093	293.15	293.15	0	362.605	362.605	0.0824232	0.0824563

357	89.64	-15.9066	20.0008	-0.0212614	1.65803	293.15	293.15	0	362.775	362.775	0.0824625	0.082496

358	89.8	-15.8698	20.0008	-0.0212111	1.66071	293.15	293.15	0	362.94	362.94	0.0825013	0.0825341

359	89.97	-15.8174	20.0008	-0.0211401	1.6647	293.15	293.15	0	363.097	363.097	0.0825396	0.0825728

360	90.14	-15.8078	20.0008	-0.0211261	1.66954	293.15	293.15	0	363.269	363.269	0.0825781	0.0826119

361	90.3	-15.8344	20.0008	-0.0211607	1.67889	293.15	293.15	0	363.441	363.441	0.0826155	0.0826495

362	90.47	-15.8322	19.9998	-0.0211567	1.6826	293.15	293.15	0	363.608	363.608	0.0826549	0.0826892

363	90.64	-15.7575	19.9904	-0.0210558	1.68856	293.15	293.15	0	363.779	363.779	0.0826928	0.0827275

364	90.8	-15.7243	19.9904	-0.0210103	1.69	293.15	293.15	0	363.945	363.945	0.0827317	0.0827661

365	90.97	-15.7208	20.006	-0.0210047	1.69557	293.15	293.15	0	364.1	364.1	0.0827714	0.0828044

366	91.14	-15.7381	20.0008	-0.0210266	1.69987	293.15	293.15	0	364.273	364.273	0.0828102	0.0828438

367	91.3	-15.7475	20.0008	-0.0210382	1.70557	293.15	293.15	0	364.437	364.437	0.0828478	0.0828816

368	91.47	-15.7359	20.0008	-0.0210216	1.70996	293.15	293.15	0	364.611	364.611	0.082886	0.0829204

369	91.64	-15.7146	20.0008	-0.0209921	1.71626	293.15	293.15	0	364.775	364.775	0.0829242	0.0829589

370	91.81	-15.706	20.0008	-0.0209796	1.72237	293.15	293.15	0	364.941	364.941	0.0829625	0.0829978

371	91.97	-15.7112	20.0008	-0.0209855	1.72501	293.15	293.15	0	365.102	365.102	0.083001	0.0830361

372	92.14	-15.7393	20.0008	-0.021022	1.72964	293.15	293.15	0	365.269	365.269	0.0830395	0.0830747

373	92.31	-15.7823	20.0008	-0.0210783	1.72517	293.15	293.15	0	365.441	365.441	0.0830797	0.0831148

374	92.77	-16.2127	20.0008	-0.0216502	1.625	293.15	293.15	0	365.613	365.613	0.0831755	0.0832194

375	92.92	-19.2126	20.0008	-0.0256551	1.63503	293.15	293.15	0	365.779	365.779	0.0832104	0.0832547

376	92.99	-19.1252	20.0008	-0.0255378	1.65569	293.15	293.15	0	365.934	365.934	0.0832329	0.0832708

377	93.08	-17.5896	20.0008	-0.0234866	1.67944	293.15	293.15	0	366.1	366.1	0.0832582	0.0832929

378	93.2	-16.1067	19.9977	-0.0215059	1.69926	293.15	293.15	0	366.269	366.269	0.0832857	0.0833189

379	93.32	-15.0554	19.9987	-0.0201014	1.72045	293.15	293.15	0	366.437	366.437	0.0833136	0.0833472

380	93.46	-14.4256	20.0008	-0.0192597	1.73759	293.15	293.15	0	366.61	366.61	0.0833454	0.0833789

381	93.6	-14.1068	20.0008	-0.0188332	1.75109	293.15	293.15	0	366.762	366.762	0.0833788	0.0834124

382	93.75	-14.0407	19.9935	-0.0187442	1.76653	293.15	293.15	0	366.931	366.931	0.0834133	0.0834472

383	93.91	-14.1502	19.9925	-0.0188895	1.77842	293.15	293.15	0	367.104	367.104	0.0834483	0.0834836

384	94.07	-14.3064	20.0008	-0.019097	1.78632	293.15	293.15	0	367.272	367.272	0.0834862	0.0835218

385	94.24	-14.5523	20.0008	-0.0194243	1.79844	293.15	293.15	0	367.441	367.441	0.0835236	0.0835596

386	94.41	-14.8487	20.0008	-0.019819	1.80523	293.15	293.15	0	367.615	367.615	0.0835623	0.0835986

387	94.58	-15.1276	20.0008	-0.0201902	1.81157	293.15	293.15	0	367.762	367.762	0.0836008	0.0836381

388	94.75	-15.3294	20.0008	-0.0204585	1.81839	293.15	293.15	0	367.928	367.928	0.0836394	0.0836766

389	94.92	-15.4969	20.0008	-0.020681	1.82358	293.15	293.15	0	368.099	368.099	0.0836796	0.0837177

390	95.1	-15.6738	20.0008	-0.020916	1.83187	293.15	293.15	0	368.272	368.272	0.0837192	0.0837575

391	95.27	-15.8366	20.0008	-0.021132	1.83613	293.15	293.15	0	368.436	368.436	0.0837587	0.0837977

392	95.44	-15.9363	20.0008	-0.021264	1.84129	293.15	293.15	0	368.602	368.602	0.0837986	0.0838376

393	95.62	-16.0762	20.0008	-0.0214496	1.84932	293.15	293.15	0	368.766	368.766	0.0838383	0.0838774

394	95.79	-16.2228	20.0008	-0.021644	1.85224	293.15	293.15	0	368.931	368.931	0.0838783	0.0839181

395	95.96	-16.2494	20.0008	-0.0216784	1.85605	293.15	293.15	0	369.104	369.104	0.0839174	0.0839571

396	96.13	-16.2343	20.0008	-0.0216572	1.8589	293.15	293.15	0	369.277	369.277	0.0839569	0.083996

397	96.31	-16.2787	20.006	-0.0217153	1.86448	293.15	293.15	0	369.441	369.441	0.0839971	0.0840366

398	96.47	-16.3013	20.0112	-0.0217444	1.87002	293.15	293.15	0	369.606	369.606	0.0840353	0.0840752

399	96.64	-16.3	20.0019	-0.0217415	1.87263	293.15	293.15	0	369.762	369.762	0.0840746	0.0841147

400	96.81	-16.323	20.0008	-0.021771	1.87569	293.15	293.15	0	369.933	369.933	0.084114	0.0841538

401	96.98	-16.3704	20.0008	-0.0218332	1.88328	293.15	293.15	0	370.099	370.099	0.0841527	0.0841928

402	97.15	-16.2991	20.0008	-0.021737	1.88667	293.15	293.15	0	370.28	370.28	0.0841923	0.0842321

403	97.32	-16.2393	19.9966	-0.0216561	1.88932	293.15	293.15	0	370.446	370.446	0.0842313	0.0842713

404	97.49	-16.18	19.9904	-0.0215759	1.89072	293.15	293.15	0	370.6	370.6	0.0842707	0.0843094

405	97.66	-16.0794	19.9935	-0.0214408	1.9012	293.15	293.15	0	370.766	370.766	0.084309	0.0843482

406	97.82	-16.0524	20.0008	-0.0214036	1.90607	293.15	293.15	0	370.936	370.936	0.0843465	0.0843865

407	97.99	-16.0805	19.9977	-0.02144	1.91031	293.15	293.15	0	371.104	371.104	0.0843851	0.0844253

408	98.16	-16.0377	19.9925	-0.0213819	1.91601	293.15	293.15	0	371.264	371.264	0.0844233	0.0844631

409	98.33	-15.9978	20.0008	-0.0213277	1.9208	293.15	293.15	0	371.433	371.433	0.0844625	0.0845026

410	98.49	-15.9768	20.0008	-0.0212985	1.92781	293.15	293.15	0	371.607	371.607	0.0845004	0.0845406

411	98.66	-15.913	20.0008	-0.0212125	1.93186	293.15	293.15	0	371.774	371.774	0.0845388	0.0845785

412	98.82	-15.8764	20.0008	-0.0211626	1.93635	293.15	293.15	0	371.935	371.935	0.0845767	0.0846172

413	98.99	-15.8537	20.0008	-0.0211313	1.94348	293.15	293.15	0	372.101	372.101	0.084614	0.0846547

414	99.16	-15.9105	20.0008	-0.021206	1.94781	293.15	293.15	0	372.267	372.267	0.0846542	0.0846941

415	99.33	-16.017	20.0008	-0.0213468	1.95264	293.15	293.15	0	372.438	372.438	0.0846921	0.0847333

416	99.5	-16.1093	20.0008	-0.0214688	1.95793	293.15	293.15	0	372.602	372.602	0.0847307	0.0847721

417	99.66	-16.1089	20.0008	-0.0214671	1.96414	293.15	293.15	0	372.775	372.775	0.0847693	0.0848108

418	99.83	-16.1274	20.0008	-0.0214908	1.9708	293.15	293.15	0	372.932	372.932	0.0848065	0.0848488

419	100	-16.1286	20.0008	-0.0214912	1.97554	293.15	293.15	0	373.096	373.096	0.0848449	0.0848874

420	100.16	-16.1282	20.0008	-0.0214896	1.88954	293.15	293.15	0	373.049	373.049	0.0848831	0.0849256

421	100.29	-16.12	20.0008	-0.0214779	1.75639	293.15	293.15	0	372.876	372.876	0.0849139	0.0849552

422	100.34	-15.5636	20.0008	-0.0207363	1.64892	293.15	293.15	0	372.712	372.712	0.0849269	0.0849658

423	100.31	-14.0319	20.0008	-0.0186957	1.55384	293.15	293.15	0	372.539	372.539	0.0849255	0.084959

424	100.22	-11.6462	20.005	-0.0155175	1.48569	293.15	293.15	0	372.384	372.384	0.0849104	0.084939

425	100.09	-8.76979	20.0071	-0.0116854	1.42534	293.15	293.15	0	372.218	372.218	0.0848848	0.0849086

426	99.92	-5.63641	20.0008	-0.00751066	1.37574	293.15	293.15	0	372.046	372.046	0.0848509	0.0848701

427	99.73	-2.59932	20.0008	-0.00346386	1.33923	293.15	293.15	0	371.881	371.881	0.0848098	0.0848251

428	99.51	0.183304	20.0008	0.000244286	1.31733	293.15	293.15	0	371.708	371.708	0.0847639	0.0847762

429	99.28	2.70142	19.9966	0.00360039	1.29656	293.15	293.15	0	371.543	371.543	0.084714	0.0847234

430	99.05	4.79083	19.9935	0.00638555	1.28214	293.15	293.15	0	371.381	371.381	0.0846628	0.0846704

431	98.82	6.4791	20.0008	0.00863641	1.2786	293.15	293.15	0	371.223	371.223	0.08461	0.0846156

432	98.58	7.80734	19.9977	0.0104076	1.27307	293.15	293.15	0	371.049	371.049	0.0845567	0.0845614

433	98.35	8.8412	19.9935	0.0117867	1.27221	293.15	293.15	0	370.885	370.885	0.0845038	0.0845076

434	98.12	9.5712	20.0008	0.0127607	1.2655	293.15	293.15	0	370.716	370.716	0.0844519	0.084455

435	97.89	10.0703	20.0008	0.0134271	1.26826	293.15	293.15	0	370.538	370.538	0.0844	0.0844031

436	97.67	10.452	20.0008	0.0139369	1.27244	293.15	293.15	0	370.378	370.378	0.0843486	0.0843512

437	97.45	10.648	20.0008	0.0141992	1.2747	293.15	293.15	0	370.218	370.218	0.0842981	0.0843009

438	97.25	10.6549	20.0008	0.0142093	1.27645	293.15	293.15	0	370.053	370.053	0.0842496	0.0842533

439	97.04	10.4824	20.0008	0.0139802	1.27972	293.15	293.15	0	369.881	369.881	0.0842027	0.0842059

440	96.85	10.2149	20.0008	0.0136241	1.28307	293.15	293.15	0	369.713	369.713	0.0841572	0.0841615

441	96.65	9.97401	20.0008	0.0133036	1.28007	293.15	293.15	0	369.544	369.544	0.0841125	0.084116

442	96.46	9.74718	20.0008	0.0130018	1.2839	293.15	293.15	0	369.378	369.378	0.0840672	0.0840722

443	96.28	9.48518	20.0008	0.012653	1.28467	293.15	293.15	0	369.223	369.223	0.0840247	0.08403

444	96.09	9.26218	20.0008	0.0123563	1.28495	293.15	293.15	0	369.057	369.057	0.0839819	0.0839868

445	95.92	9.01064	20.0019	0.0120213	1.28035	293.15	293.15	0	368.877	368.877	0.0839417	0.0839468

446	95.73	8.77048	19.9987	0.0117015	1.27954	293.15	293.15	0	368.711	368.711	0.0839003	0.0839047

447	95.56	8.60537	19.9904	0.0114819	1.27707	293.15	293.15	0	368.539	368.539	0.08386	0.0838642

448	95.39	8.44789	19.9904	0.0112723	1.27271	293.15	293.15	0	368.381	368.381	0.0838204	0.0838248

449	95.21	8.26504	20.006	0.0110289	1.26771	293.15	293.15	0	368.219	368.219	0.0837807	0.0837849

450	95.05	8.12259	20.0112	0.0108394	1.26439	293.15	293.15	0	368.054	368.054	0.0837415	0.083746

451	94.87	7.97869	19.9904	0.0106479	1.26514	293.15	293.15	0	367.881	367.881	0.0837019	0.0837064

452	94.71	7.87889	20.0008	0.0105152	1.25955	293.15	293.15	0	367.708	367.708	0.0836642	0.083668

453	94.54	7.75563	20.0008	0.0103512	1.25273	293.15	293.15	0	367.544	367.544	0.0836252	0.0836299

454	94.37	7.67674	20.0008	0.0102465	1.25176	293.15	293.15	0	367.377	367.377	0.0835855	0.0835901

455	94.21	7.67384	20.0008	0.0102431	1.24754	293.15	293.15	0	367.216	367.216	0.0835474	0.0835521

456	94.04	7.6571	20.0008	0.0102213	1.24431	293.15	293.15	0	367.05	367.05	0.0835092	0.0835136

457	93.87	7.68507	19.9956	0.0102591	1.23892	293.15	293.15	0	366.876	366.876	0.0834705	0.0834748

458	93.71	7.64772	20.0008	0.0102098	1.23336	293.15	293.15	0	366.705	366.705	0.0834331	0.0834366

459	93.54	7.60338	20.0008	0.0101511	1.22926	293.15	293.15	0	366.539	366.539	0.0833945	0.0833981

460	93.37	7.58213	19.9977	0.0101232	1.22725	293.15	293.15	0	366.384	366.384	0.0833554	0.0833588

461	93.2	7.54772	19.9935	0.0100778	1.22015	293.15	293.15	0	366.219	366.219	0.0833175	0.0833207

462	93.03	7.51675	20.0008	0.0100369	1.21342	293.15	293.15	0	366.05	366.05	0.083279	0.0832817

463	92.87	7.46276	19.9956	0.00996534	1.20846	293.15	293.15	0	365.881	365.881	0.0832408	0.0832439

464	92.71	7.47119	20.0008	0.00997708	1.20436	293.15	293.15	0	365.702	365.702	0.0832023	0.0832057

465	92.54	7.52875	20.0008	0.0100545	1.20048	293.15	293.15	0	365.543	365.543	0.0831633	0.0831669

466	92.37	7.53267	20.0008	0.0100602	1.19375	293.15	293.15	0	365.383	365.383	0.0831251	0.0831282

467	92.21	7.51327	20.0008	0.0100348	1.1897	293.15	293.15	0	365.222	365.222	0.0830872	0.08309

468	92.04	7.53094	20.0008	0.0100589	1.18468	293.15	293.15	0	365.047	365.047	0.0830485	0.083051

469	91.87	7.5755	20.0008	0.0101189	1.17761	293.15	293.15	0	364.875	364.875	0.0830098	0.0830122

470	91.7	7.55982	20.0008	0.0100985	1.17206	293.15	293.15	0	364.709	364.709	0.0829718	0.0829737

471	91.53	7.5501	20.0008	0.010086	1.16752	293.15	293.15	0	364.554	364.554	0.0829333	0.0829351

472	91.36	7.5697	19.9956	0.0101127	1.16711	293.15	293.15	0	364.39	364.39	0.0828938	0.0828957

473	91.2	7.55183	19.9904	0.0100893	1.16227	293.15	293.15	0	364.217	364.217	0.0828561	0.0828579

474	91.03	7.57915	19.9956	0.0101263	1.15602	293.15	293.15	0	364.044	364.044	0.0828174	0.0828192

475	90.87	7.63781	20.0008	0.0102052	1.1502	293.15	293.15	0	363.88	363.88	0.0827792	0.0827806

476	90.7	7.61857	20.0008	0.01018	1.14735	293.15	293.15	0	363.707	363.707	0.0827402	0.0827413

477	90.53	7.6132	19.9956	0.0101734	1.14396	293.15	293.15	0	363.552	363.552	0.0827019	0.0827031

478	90.37	7.68778	20.0008	0.0102735	1.13678	293.15	293.15	0	363.386	363.386	0.0826635	0.0826647

479	90.2	7.72864	20.0008	0.0103287	1.13216	293.15	293.15	0	363.213	363.213	0.082625	0.0826255

480	90.03	7.78046	20.0008	0.0103984	1.12866	293.15	293.15	0	363.042	363.042	0.0825865	0.0825874

481	89.87	7.78828	19.9966	0.0104094	1.12297	293.15	293.15	0	362.875	362.875	0.0825484	0.0825492

482	89.7	7.79614	19.9935	0.0104204	1.11555	293.15	293.15	0	362.71	362.71	0.0825097	0.0825105

483	89.53	7.75893	20.0008	0.0103712	1.11326	293.15	293.15	0	362.555	362.555	0.0824707	0.082471

484	89.36	7.7587	19.9977	0.0103714	1.1075	293.15	293.15	0	362.385	362.385	0.0824316	0.0824314

485	89.19	7.80706	19.9935	0.0104366	1.10263	293.15	293.15	0	362.217	362.217	0.0823937	0.0823929

486	89.02	7.78665	20.0008	0.0104099	1.09864	293.15	293.15	0	362.044	362.044	0.0823551	0.0823541

487	88.85	7.75241	20.0008	0.0103646	1.09446	293.15	293.15	0	361.875	361.875	0.0823156	0.082315

488	88.69	7.75497	20.0008	0.0103685	1.09106	293.15	293.15	0	361.715	361.715	0.082277	0.0822765

489	88.52	7.77395	20.0008	0.0103944	1.0886	293.15	293.15	0	361.55	361.55	0.0822376	0.0822374

490	88.35	7.76951	20.0008	0.010389	1.08079	293.15	293.15	0	361.383	361.383	0.0821995	0.0821984

491	88.18	7.73525	20.0008	0.0103437	1.07828	293.15	293.15	0	361.213	361.213	0.0821605	0.0821594

492	88.01	7.72162	20.0008	0.0103261	1.07332	293.15	293.15	0	361.049	361.049	0.0821227	0.0821205

493	87.85	7.73179	20.0008	0.0103402	1.06767	293.15	293.15	0	360.876	360.876	0.0820851	0.0820829

494	87.68	7.7028	20.0008	0.0103019	1.06287	293.15	293.15	0	360.708	360.708	0.0820454	0.0820439

495	87.51	7.70747	20.0008	0.0103087	1.05867	293.15	293.15	0	360.555	360.555	0.0820074	0.0820053

496	87.35	7.72585	20.0008	0.0103338	1.05342	293.15	293.15	0	360.382	360.382	0.0819694	0.081967

497	87.18	7.75697	20.0008	0.0103759	1.04906	293.15	293.15	0	360.218	360.218	0.0819294	0.0819267

498	87.01	7.73851	20.0008	0.0103517	1.04426	293.15	293.15	0	360.052	360.052	0.0818916	0.0818887

499	86.84	7.69714	20.0008	0.0102969	1.03967	293.15	293.15	0	359.88	359.88	0.0818527	0.0818497

500	86.67	7.67602	20.0008	0.0102692	1.03573	293.15	293.15	0	359.707	359.707	0.0818136	0.0818103

501	86.51	7.74395	20.0008	0.0103606	1.02886	293.15	293.15	0	359.56	359.56	0.0817757	0.081772

502	86.34	7.76617	20.0008	0.0103908	1.02599	293.15	293.15	0	359.386	359.386	0.0817364	0.0817333

503	86.17	7.79627	20.0008	0.0104316	1.0201	293.15	293.15	0	359.223	359.223	0.0816987	0.0816946

504	86	7.84456	20.0008	0.0104968	1.02032	293.15	293.15	0	359.049	359.049	0.0816591	0.0816555

505	85.84	7.83976	19.9904	0.0104909	1.00936	293.15	293.15	0	358.876	358.876	0.0816215	0.0816177

506	85.67	7.75002	19.9904	0.0103713	1.00648	293.15	293.15	0	358.703	358.703	0.0815828	0.0815784

507	85.51	7.73605	19.9956	0.0103531	1.00489	293.15	293.15	0	358.556	358.556	0.0815435	0.0815401

508	85.34	7.73781	19.9946	0.010356	0.999917	293.15	293.15	0	358.382	358.382	0.0815054	0.0815012

509	85.17	7.76645	20.0008	0.0103949	0.996927	293.15	293.15	0	358.211	358.211	0.0814665	0.0814617

510	85	7.82673	20.0008	0.0104761	0.989391	293.15	293.15	0	358.045	358.045	0.0814278	0.0814223

511	84.83	7.87966	20.0008	0.0105475	0.986226	293.15	293.15	0	357.872	357.872	0.0813898	0.0813845

512	84.66	7.8922	20.0008	0.0105648	0.982334	293.15	293.15	0	357.709	357.709	0.0813503	0.0813451

513	84.5	7.97318	19.9956	0.0106737	0.977468	293.15	293.15	0	357.551	357.551	0.0813114	0.0813068

514	84.33	8.01998	20.0008	0.0107369	0.972026	293.15	293.15	0	357.378	357.378	0.0812727	0.0812676

515	84.17	8.01698	20.0008	0.0107334	0.96594	293.15	293.15	0	357.214	357.214	0.0812357	0.0812294

516	83.99	7.96312	20.0008	0.0106619	0.9642	293.15	293.15	0	357.044	357.044	0.081195	0.0811895

517	83.83	7.94175	19.9977	0.0106338	0.960444	293.15	293.15	0	356.876	356.876	0.0811567	0.0811511

518	83.66	7.86209	19.9904	0.0105277	0.95088	293.15	293.15	0	356.71	356.71	0.0811192	0.081113

519	83.5	7.82711	19.9925	0.0104813	0.949075	293.15	293.15	0	356.552	356.552	0.0810799	0.081074

520	83.33	7.8837	20.0008	0.0105577	0.94695	293.15	293.15	0	356.383	356.383	0.0810409	0.0810347

521	83.16	7.94586	20.0008	0.0106414	0.943105	293.15	293.15	0	356.209	356.209	0.0810017	0.0809957

522	82.99	7.93585	19.9987	0.0106286	0.937797	293.15	293.15	0	356.042	356.042	0.0809633	0.0809572

523	82.82	7.90857	19.9925	0.0105926	0.933922	293.15	293.15	0	355.872	355.872	0.080925	0.0809183

524	82.65	7.95617	20.0008	0.0106569	0.929915	293.15	293.15	0	355.716	355.716	0.0808865	0.0808789

525	82.49	8.04876	20.0008	0.0107814	0.924661	293.15	293.15	0	355.55	355.55	0.0808478	0.0808405

526	82.31	8.15165	20.0008	0.0109198	0.919877	293.15	293.15	0	355.385	355.385	0.0808082	0.0808

527	82.15	8.23239	20.0008	0.0110285	0.915084	293.15	293.15	0	355.213	355.213	0.0807703	0.0807628

528	81.99	8.25766	20.0008	0.0110629	0.910235	293.15	293.15	0	355.04	355.04	0.0807319	0.0807244

529	81.82	8.26721	20.0008	0.0110763	0.904298	293.15	293.15	0	354.875	354.875	0.0806929	0.0806848

530	81.65	8.28268	20.0008	0.0110976	0.900699	293.15	293.15	0	354.71	354.71	0.0806537	0.0806457

531	81.48	8.3383	20.0008	0.0111726	0.897849	293.15	293.15	0	354.547	354.547	0.0806152	0.0806072

532	81.31	8.38291	20.0008	0.011233	0.893849	293.15	293.15	0	354.38	354.38	0.0805769	0.0805679

533	81.15	8.34714	20.0008	0.0111856	0.89155	293.15	293.15	0	354.219	354.219	0.0805379	0.0805289

534	80.98	8.30949	20.0008	0.0111357	0.887268	293.15	293.15	0	354.052	354.052	0.0804982	0.0804899

535	80.81	8.25453	20.0008	0.0110626	0.881614	293.15	293.15	0	353.88	353.88	0.0804595	0.0804504

536	80.65	8.2023	20.0008	0.0109932	0.877509	293.15	293.15	0	353.708	353.708	0.0804223	0.080413

537	80.48	8.22555	20.0008	0.0110249	0.87173	293.15	293.15	0	353.542	353.542	0.0803836	0.0803739

538	80.31	8.27888	20.0008	0.0110969	0.866737	293.15	293.15	0	353.377	353.377	0.0803456	0.0803357

539	80.15	8.26705	19.9977	0.0110816	0.863511	293.15	293.15	0	353.216	353.216	0.0803059	0.080297

540	79.98	8.27002	19.9967	0.0110862	0.858455	293.15	293.15	0	353.047	353.047	0.0802674	0.0802577

541	79.81	8.27531	20.0081	0.0110938	0.853484	293.15	293.15	0	352.874	352.874	0.0802289	0.0802187

542	79.64	8.36865	19.9987	0.0112195	0.84839	293.15	293.15	0	352.714	352.714	0.0801902	0.0801791

543	79.47	8.44105	19.9904	0.0113172	0.844384	293.15	293.15	0	352.554	352.554	0.0801513	0.0801405

544	79.3	8.46195	19.9977	0.0113458	0.842135	293.15	293.15	0	352.381	352.381	0.0801117	0.0801002

545	79.14	8.45976	20.0008	0.0113434	0.839139	293.15	293.15	0	352.217	352.217	0.0800738	0.0800627

546	78.97	8.45179	20.0008	0.0113333	0.831433	293.15	293.15	0	352.049	352.049	0.0800348	0.0800236

547	78.8	8.43684	20.0008	0.0113138	0.829852	293.15	293.15	0	351.871	351.871	0.0799955	0.0799849

548	78.64	8.45043	20.0008	0.0113326	0.827389	293.15	293.15	0	351.714	351.714	0.0799566	0.0799463

549	78.47	8.4292	20.0008	0.0113047	0.823291	293.15	293.15	0	351.557	351.557	0.0799178	0.0799067

550	78.3	8.35269	20.0008	0.0112027	0.818013	293.15	293.15	0	351.386	351.386	0.0798799	0.0798677

551	78.13	8.26855	20.0008	0.0110904	0.813263	293.15	293.15	0	351.213	351.213	0.0798408	0.0798291

552	77.96	8.24895	20.0008	0.0110646	0.806823	293.15	293.15	0	351.047	351.047	0.0798024	0.0797902

553	77.8	8.25316	20.0008	0.0110708	0.803158	293.15	293.15	0	350.875	350.875	0.0797637	0.0797517

554	77.63	8.26631	20.0008	0.011089	0.798834	293.15	293.15	0	350.709	350.709	0.0797244	0.0797127

555	77.46	8.30096	20.0008	0.0111361	0.793426	293.15	293.15	0	350.554	350.554	0.0796861	0.0796737

556	77.29	8.32521	20.0008	0.0111692	0.792414	293.15	293.15	0	350.39	350.39	0.0796469	0.079634

557	77.13	8.34135	20.0008	0.0111914	0.786612	293.15	293.15	0	350.217	350.217	0.0796086	0.0795957

558	76.96	8.37384	20.006	0.0112356	0.782218	293.15	293.15	0	350.044	350.044	0.0795688	0.0795562

559	76.79	8.4049	20.0112	0.0112778	0.779289	293.15	293.15	0	349.88	349.88	0.0795304	0.0795178

560	76.62	8.42919	20.0008	0.011311	0.773786	293.15	293.15	0	349.714	349.714	0.0794923	0.0794789

561	76.46	8.37746	19.9966	0.0112421	0.77173	293.15	293.15	0	349.552	349.552	0.0794536	0.0794407

562	76.29	8.30963	19.9904	0.0111516	0.766587	293.15	293.15	0	349.385	349.385	0.0794152	0.0794019

563	76.12	8.28507	19.9998	0.0111192	0.761779	293.15	293.15	0	349.213	349.213	0.0793763	0.0793626

564	75.96	8.32518	20.0008	0.0111736	0.759134	293.15	293.15	0	349.041	349.041	0.0793371	0.0793232

565	75.79	8.3446	20.0008	0.0112003	0.756058	293.15	293.15	0	348.876	348.876	0.0792984	0.0792839

566	75.62	8.36364	20.0008	0.0112264	0.749168	293.15	293.15	0	348.71	348.71	0.0792593	0.0792453

567	75.45	8.38433	20.0008	0.0112548	0.746139	293.15	293.15	0	348.549	348.549	0.0792198	0.0792055

568	75.28	8.39258	20.0008	0.0112664	0.743464	293.15	293.15	0	348.381	348.381	0.079181	0.0791664

569	75.11	8.44592	20.0008	0.0113386	0.738139	293.15	293.15	0	348.208	348.208	0.0791423	0.0791272

570	74.95	8.50828	20.0008	0.0114229	0.732148	293.15	293.15	0	348.039	348.039	0.079104	0.079089

571	74.78	8.5222	20.0008	0.0114421	0.728635	293.15	293.15	0	347.887	347.887	0.0790648	0.0790503

572	74.61	8.51687	19.9987	0.0114356	0.725421	293.15	293.15	0	347.714	347.714	0.0790261	0.0790106

573	74.45	8.47689	19.9925	0.0113824	0.7215	293.15	293.15	0	347.55	347.55	0.0789875	0.0789725

574	74.28	8.3719	20.0008	0.011242	0.715114	293.15	293.15	0	347.382	347.382	0.0789491	0.0789338

575	74.12	8.27616	20.0008	0.011114	0.713132	293.15	293.15	0	347.213	347.213	0.0789101	0.0788953

576	73.95	8.24693	20.0008	0.0110753	0.708855	293.15	293.15	0	347.047	347.047	0.0788716	0.0788558

577	73.78	8.22476	19.9946	0.0110461	0.706894	293.15	293.15	0	346.89	346.89	0.0788319	0.0788161

578	73.61	8.23498	19.9914	0.0110604	0.703076	293.15	293.15	0	346.719	346.719	0.0787929	0.0787769

579	73.44	8.2227	20.0008	0.0110445	0.698232	293.15	293.15	0	346.546	346.546	0.0787539	0.0787379

580	73.28	8.19324	20.0008	0.0110054	0.693653	293.15	293.15	0	346.38	346.38	0.078716	0.0787

581	73.11	8.20018	20.0008	0.0110153	0.690177	293.15	293.15	0	346.209	346.209	0.0786763	0.0786603

582	72.94	8.27722	20.0008	0.0111194	0.682654	293.15	293.15	0	346.042	346.042	0.078638	0.0786208

583	72.77	8.31854	20.0008	0.0111755	0.679028	293.15	293.15	0	345.888	345.888	0.0785992	0.0785824

584	72.61	8.34858	20.0008	0.0112164	0.674882	293.15	293.15	0	345.713	345.713	0.0785606	0.0785436

585	72.44	8.40145	20.0008	0.011288	0.673626	293.15	293.15	0	345.542	345.542	0.0785221	0.0785054

586	72.27	8.44353	20.0008	0.0113451	0.671456	293.15	293.15	0	345.367	345.367	0.0784828	0.0784659

587	72.11	8.45262	20.0008	0.0113579	0.664476	293.15	293.15	0	345.211	345.211	0.0784443	0.0784276

588	71.94	8.46615	19.9966	0.0113766	0.661477	293.15	293.15	0	345.039	345.039	0.0784055	0.0783886

589	71.77	8.49504	19.9935	0.011416	0.65842	293.15	293.15	0	344.891	344.891	0.0783665	0.0783489

590	71.6	8.54288	20.0008	0.0114809	0.654723	293.15	293.15	0	344.721	344.721	0.0783276	0.0783105

591	71.43	8.59218	20.0008	0.0115477	0.648684	293.15	293.15	0	344.545	344.545	0.0782883	0.0782705

592	71.27	8.62589	20.0008	0.0115936	0.643928	293.15	293.15	0	344.375	344.375	0.0782493	0.0782316

593	71.1	8.63911	20.0008	0.011612	0.639907	293.15	293.15	0	344.206	344.206	0.078211	0.0781932

594	70.93	8.66108	20.0008	0.0116421	0.637147	293.15	293.15	0	344.042	344.042	0.0781721	0.0781538

595	70.77	8.69017	20.0008	0.0116818	0.62938	293.15	293.15	0	343.886	343.886	0.0781337	0.0781153

596	70.6	8.68532	20.0008	0.0116759	0.626845	293.15	293.15	0	343.718	343.718	0.0780945	0.0780765

597	70.43	8.63968	19.9987	0.0116151	0.624099	293.15	293.15	0	343.549	343.549	0.0780554	0.0780362

598	70.26	8.63087	19.9925	0.0116038	0.620811	293.15	293.15	0	343.376	343.376	0.0780168	0.0779979

599	70.09	8.64453	20.0008	0.0116228	0.615263	293.15	293.15	0	343.208	343.208	0.0779779	0.0779581

600	69.93	8.63997	20.0008	0.0116173	0.612269	293.15	293.15	0	343.047	343.047	0.0779392	0.0779195

601	69.75	8.62921	20.0008	0.0116034	0.610344	293.15	293.15	0	342.882	342.882	0.0778996	0.0778793

602	69.59	8.62941	20.0008	0.0116042	0.604645	293.15	293.15	0	342.716	342.716	0.0778614	0.0778407

603	69.42	8.65844	20.0008	0.0116439	0.598345	293.15	293.15	0	342.545	342.545	0.0778223	0.0778017

604	69.25	8.73343	20.0008	0.0117453	0.594551	293.15	293.15	0	342.371	342.371	0.0777833	0.0777627

605	69.09	8.86097	20.0008	0.0119174	0.593658	293.15	293.15	0	342.207	342.207	0.0777436	0.0777233

606	68.92	8.92788	20.0008	0.012008	0.587378	293.15	293.15	0	342.06	342.06	0.0777052	0.0776846

607	68.75	8.9489	20.0008	0.0120369	0.58238	293.15	293.15	0	341.886	341.886	0.0776661	0.0776449

608	68.59	8.96738	20.0008	0.0120624	0.580143	293.15	293.15	0	341.713	341.713	0.0776275	0.0776066

609	68.42	8.9093	20.0008	0.0119849	0.578034	293.15	293.15	0	341.547	341.547	0.0775881	0.0775671

610	68.25	8.85743	20.0008	0.0119157	0.572041	293.15	293.15	0	341.376	341.376	0.0775489	0.0775281

611	68.08	8.80928	20.0008	0.0118515	0.568596	293.15	293.15	0	341.203	341.203	0.0775104	0.0774895

612	67.92	8.73533	20.0008	0.0117526	0.565688	293.15	293.15	0	341.048	341.048	0.0774718	0.0774508

613	67.75	8.68896	20.0008	0.0116908	0.56444	293.15	293.15	0	340.882	340.882	0.0774325	0.0774115

614	67.58	8.69373	20.0008	0.0116978	0.561336	293.15	293.15	0	340.718	340.718	0.0773935	0.0773721

615	67.41	8.74877	20.0008	0.0117725	0.555065	293.15	293.15	0	340.545	340.545	0.0773556	0.0773334

616	67.25	8.81076	20.0008	0.0118565	0.549879	293.15	293.15	0	340.381	340.381	0.0773169	0.0772946

617	67.08	8.84806	20.0008	0.0119073	0.546364	293.15	293.15	0	340.207	340.207	0.0772773	0.0772546

618	66.91	8.91842	20.0008	0.0120026	0.542887	293.15	293.15	0	340.036	340.036	0.0772391	0.0772161

619	66.74	9.02451	20.0008	0.012146	0.540589	293.15	293.15	0	339.887	339.887	0.0771991	0.0771762

620	66.57	9.09725	20.0008	0.0122445	0.535227	293.15	293.15	0	339.713	339.713	0.0771604	0.0771373

621	66.41	9.14366	20.0008	0.0123076	0.531316	293.15	293.15	0	339.544	339.544	0.0771216	0.0770979

622	66.24	9.06747	20.0008	0.0122057	0.529043	293.15	293.15	0	339.376	339.376	0.0770816	0.0770586

623	66.07	8.96543	20.0008	0.0120689	0.521461	293.15	293.15	0	339.203	339.203	0.0770435	0.0770204

624	65.91	8.9262	20.0008	0.0120167	0.518679	293.15	293.15	0	339.043	339.043	0.0770044	0.0769814

625	65.74	9.00176	20.0008	0.012119	0.515807	293.15	293.15	0	338.882	338.882	0.0769664	0.0769421

626	65.57	9.10132	20.0029	0.0122537	0.511594	293.15	293.15	0	338.718	338.718	0.076927	0.0769025

627	65.4	9.16077	20.0112	0.0123344	0.508467	293.15	293.15	0	338.545	338.545	0.0768878	0.0768629

628	65.23	9.16818	20.0091	0.012345	0.505995	293.15	293.15	0	338.377	338.377	0.0768484	0.0768238

629	65.06	9.16962	19.9998	0.0123475	0.502608	293.15	293.15	0	338.224	338.224	0.0768094	0.0767844

630	64.9	9.23034	19.9966	0.0124299	0.497997	293.15	293.15	0	338.051	338.051	0.0767709	0.0767455

631	64.73	9.29802	20.0008	0.0125217	0.492311	293.15	293.15	0	337.885	337.885	0.0767322	0.0767063

632	64.57	9.25345	20.0008	0.0124623	0.489382	293.15	293.15	0	337.714	337.714	0.0766935	0.0766681

633	64.4	9.21221	20.0008	0.0124074	0.483051	293.15	293.15	0	337.541	337.541	0.0766552	0.0766292

634	64.23	9.22926	20.0008	0.012431	0.479788	293.15	293.15	0	337.375	337.375	0.0766153	0.0765897

635	64.06	9.27147	20.0008	0.0124885	0.47693	293.15	293.15	0	337.22	337.22	0.0765762	0.0765506

636	63.89	9.2654	20.0008	0.0124809	0.472938	293.15	293.15	0	337.047	337.047	0.0765373	0.0765113

637	63.73	9.22093	20.0008	0.0124217	0.470297	293.15	293.15	0	336.882	336.882	0.0764982	0.0764718

638	63.56	9.19293	19.9956	0.0123846	0.466344	293.15	293.15	0	336.709	336.709	0.0764587	0.0764328

639	63.39	9.13384	19.9956	0.0123056	0.464397	293.15	293.15	0	336.545	336.545	0.0764194	0.0763938

640	63.23	9.10248	20.0008	0.0122639	0.459561	293.15	293.15	0	336.381	336.381	0.0763817	0.0763559

641	63.06	9.13778	20.0008	0.0123121	0.456424	293.15	293.15	0	336.215	336.215	0.0763426	0.0763159

642	62.89	9.21873	20.0008	0.0124219	0.45495	293.15	293.15	0	336.044	336.044	0.0763033	0.0762761

643	62.72	9.26903	20.0008	0.0124903	0.44881	293.15	293.15	0	335.878	335.878	0.0762641	0.0762368

644	62.55	9.26496	20.0008	0.0124854	0.447148	293.15	293.15	0	335.705	335.705	0.0762245	0.0761979

645	62.39	9.31348	20.0008	0.0125514	0.441491	293.15	293.15	0	335.557	335.557	0.0761862	0.0761587

646	62.22	9.36927	20.0008	0.0126273	0.440198	293.15	293.15	0	335.388	335.388	0.0761469	0.0761191

647	62.05	9.35075	20.0008	0.0126029	0.432621	293.15	293.15	0	335.211	335.211	0.0761079	0.0760805

648	61.88	9.40305	20.0008	0.0126741	0.428542	293.15	293.15	0	335.041	335.041	0.0760694	0.0760415

649	61.71	9.46353	20.0008	0.0127562	0.426277	293.15	293.15	0	334.873	334.873	0.0760299	0.0760015

650	61.55	9.48788	20.0008	0.0127897	0.424347	293.15	293.15	0	334.708	334.708	0.0759913	0.0759633

651	61.38	9.4946	20.0008	0.0127994	0.416982	293.15	293.15	0	334.553	334.553	0.0759523	0.0759235

652	61.22	9.48798	20.0008	0.0127911	0.415188	293.15	293.15	0	334.376	334.376	0.075913	0.0758848

653	61.05	9.53529	20.0008	0.0128556	0.412022	293.15	293.15	0	334.207	334.207	0.0758746	0.0758455

654	60.88	9.61724	20.0008	0.0129667	0.409917	293.15	293.15	0	334.048	334.048	0.0758348	0.0758059

655	60.71	9.62946	20.0008	0.0129838	0.403299	293.15	293.15	0	333.886	333.886	0.0757966	0.0757666

656	60.54	9.67506	20.0008	0.013046	0.401091	293.15	293.15	0	333.712	333.712	0.0757574	0.0757272

657	60.37	9.69428	20.0008	0.0130726	0.397308	293.15	293.15	0	333.549	333.549	0.0757178	0.0756881

658	60.21	9.67404	20.0008	0.0130459	0.392207	293.15	293.15	0	333.383	333.383	0.0756789	0.0756497

659	60.04	9.63764	20.0008	0.0129975	0.389609	293.15	293.15	0	333.211	333.211	0.0756397	0.0756105

660	59.87	9.62603	20.0008	0.0129825	0.385328	293.15	293.15	0	333.046	333.046	0.0756008	0.0755709

661	59.71	9.59981	20.0008	0.0129478	0.384633	293.15	293.15	0	332.89	332.89	0.0755619	0.0755319

662	59.54	9.55638	20.0008	0.0128899	0.379179	293.15	293.15	0	332.717	332.717	0.0755236	0.0754937

663	59.37	9.54767	20.0008	0.0128788	0.373565	293.15	293.15	0	332.544	332.544	0.0754833	0.0754533

664	59.2	9.56205	20.0008	0.0128988	0.372301	293.15	293.15	0	332.38	332.38	0.0754439	0.0754141

665	59.04	9.54123	20.0008	0.0128714	0.37047	293.15	293.15	0	332.216	332.216	0.0754058	0.0753755

666	58.87	9.46317	20.0008	0.0127668	0.363754	293.15	293.15	0	332.043	332.043	0.0753663	0.0753359

667	58.71	9.47302	20.0008	0.0127807	0.362463	293.15	293.15	0	331.887	331.887	0.0753276	0.0752975

668	58.54	9.53941	20.0008	0.0128709	0.357956	293.15	293.15	0	331.722	331.722	0.0752888	0.075258

669	58.37	9.52818	20.0008	0.0128564	0.356019	293.15	293.15	0	331.549	331.549	0.0752488	0.0752184

670	58.2	9.47623	20.0008	0.0127869	0.353462	293.15	293.15	0	331.377	331.377	0.0752106	0.0751799

671	58.04	9.44712	20.0008	0.0127483	0.346102	293.15	293.15	0	331.212	331.212	0.0751717	0.0751405

672	57.87	9.45377	20.0008	0.0127579	0.342555	293.15	293.15	0	331.038	331.038	0.0751336	0.0751014

673	57.7	9.46071	20.0008	0.012768	0.341719	293.15	293.15	0	330.89	330.89	0.0750936	0.0750619

674	57.53	9.61315	20.0008	0.0129744	0.334335	293.15	293.15	0	330.72	330.72	0.0750546	0.0750217

675	57.37	11.0612	20.0008	0.0149293	0.305662	293.15	293.15	0	330.553	330.553	0.0750274	0.0749855

676	57.25	15.9292	20.0008	0.0215006	0.25161	293.15	293.15	0	330.38	330.38	0.0750132	0.0749559

677	57.13	22.922	20.0008	0.0309404	0.201638	293.15	293.15	0	330.21	330.21	0.0749957	0.0749272

678	56.99	29.9267	20.0008	0.0403971	0.15686	293.15	293.15	0	330.043	330.043	0.0749724	0.0748945

679	56.82	36.9069	20.0008	0.0498219	0.119509	293.15	293.15	0	329.87	329.87	0.0749443	0.0748562

680	56.65	43.5466	20.0008	0.0587882	0.0882828	293.15	293.15	0	329.71	329.71	0.0749124	0.0748162

681	56.47	49.9618	20.0008	0.0674525	0.0607868	293.15	293.15	0	329.549	329.549	0.0748777	0.0747734

682	56.28	55.8385	19.9987	0.0753907	0.0358258	293.15	293.15	0	329.385	329.385	0.0748405	0.0747293

683	56.08	61.685	19.9977	0.0832895	0.00928002	293.15	293.15	0	329.212	329.212	0.0748025	0.0746828

684	55.88	67.315	19.9987	0.0908968	-0.00996016	293.15	293.15	0	329.044	329.044	0.0747627	0.0746363

685	55.69	72.5061	19.9925	0.0979123	-0.0298987	293.15	293.15	0	328.875	328.875	0.0747221	0.0745904

686	55.5	76.8124	20.0008	0.103733	-0.0524295	293.15	293.15	0	328.708	328.708	0.0746821	0.0745471

687	55.33	80.4877	20.0008	0.108702	-0.0782493	293.15	293.15	0	328.554	328.554	0.0746454	0.0745062

688	55.17	83.418	20.0008	0.112666	-0.105475	293.15	293.15	0	328.388	328.388	0.0746094	0.0744678

689	55	85.6068	20.0008	0.115628	-0.132577	293.15	293.15	0	328.217	328.217	0.0745714	0.074429

690	54.84	87.1912	20.0008	0.117773	-0.163855	293.15	293.15	0	328.043	328.043	0.0745352	0.0743917

691	54.68	88.3074	20.0008	0.119287	-0.192124	293.15	293.15	0	327.877	327.877	0.0744982	0.0743544

692	54.53	89.0054	20.0008	0.120235	-0.222854	293.15	293.15	0	327.716	327.716	0.0744623	0.074319

693	54.38	89.3358	20.0008	0.120687	-0.251203	293.15	293.15	0	327.548	327.548	0.0744257	0.0742828

694	54.22	89.3743	20.0008	0.120745	-0.282663	293.15	293.15	0	327.385	327.385	0.0743883	0.0742461

695	54.06	89.1013	20.0008	0.120382	-0.307568	293.15	293.15	0	327.221	327.221	0.0743505	0.0742091

696	53.91	88.5732	20.0008	0.119674	-0.33722	293.15	293.15	0	327.047	327.047	0.0743122	0.0741724

697	53.75	87.6996	20.006	0.118499	-0.364825	293.15	293.15	0	326.875	326.875	0.0742741	0.0741361

698	53.59	86.5097	20.0071	0.116897	-0.3908	293.15	293.15	0	326.72	326.72	0.0742339	0.0740978

699	53.43	85.0667	20.0008	0.114953	-0.411014	293.15	293.15	0	326.554	326.554	0.0741928	0.0740594

700	53.26	83.4462	20.0008	0.112769	-0.42933	293.15	293.15	0	326.382	326.382	0.0741496	0.0740194

701	53.08	81.553	20.0008	0.110216	-0.443645	293.15	293.15	0	326.217	326.217	0.074106	0.0739782

702	52.9	79.3526	19.9966	0.107249	-0.456506	293.15	293.15	0	326.043	326.043	0.0740591	0.0739355

703	52.71	76.9186	19.9946	0.103965	-0.462739	293.15	293.15	0	325.879	325.879	0.0740118	0.0738916

704	52.51	74.2079	20.0008	0.100307	-0.460993	293.15	293.15	0	325.717	325.717	0.0739617	0.0738448

705	52.3	71.1906	19.9977	0.0962346	-0.452061	293.15	293.15	0	325.559	325.559	0.0739079	0.0737962

706	52.09	67.7808	19.9935	0.0916314	-0.437614	293.15	293.15	0	325.386	325.386	0.0738506	0.0737449

707	51.85	63.8639	20.0008	0.0863422	-0.411854	293.15	293.15	0	325.214	325.214	0.0737898	0.0736906

708	51.61	59.5241	19.9935	0.0804809	-0.373633	293.15	293.15	0	325.052	325.052	0.0737259	0.0736333

709	51.35	54.7393	19.9925	0.0740174	-0.320299	293.15	293.15	0	324.883	324.883	0.0736578	0.0735722

710	51.08	49.7765	20.0008	0.0673123	-0.258156	293.15	293.15	0	324.709	324.709	0.0735866	0.0735079

711	50.8	45.0357	20.0008	0.0609066	-0.192919	293.15	293.15	0	324.541	324.541	0.073516	0.0734422

712	50.51	40.7053	20.0008	0.055055	-0.117942	293.15	293.15	0	324.381	324.381	0.0734436	0.0733739

713	50.23	37.2101	19.9946	0.0503319	-0.0441055	293.15	293.15	0	324.213	324.213	0.0733748	0.0733077

714	49.93	34.3089	19.9966	0.0464118	0.037364	293.15	293.15	0	324.051	324.051	0.0733049	0.0732386

715	49.66	31.8535	20.0008	0.0430938	0.112754	293.15	293.15	0	323.885	323.885	0.0732381	0.0731746

716	49.45	29.467	19.9956	0.0398676	0.174589	293.15	293.15	0	323.72	323.72	0.073185	0.0731264

717	49.3	26.5669	20.0008	0.0359456	0.221331	293.15	293.15	0	323.548	323.548	0.0731437	0.0730899

718	49.18	23.2216	20.0008	0.0314204	0.250805	293.15	293.15	0	323.375	323.375	0.0731108	0.0730628

719	49.08	19.6744	19.9956	0.0266217	0.266299	293.15	293.15	0	323.211	323.211	0.0730832	0.0730393

720	49	16.3711	20.0008	0.0221524	0.275276	293.15	293.15	0	323.046	323.046	0.0730592	0.0730197

721	48.92	13.337	20.0008	0.0180473	0.277474	293.15	293.15	0	322.89	322.89	0.0730376	0.0730005

722	48.84	10.8312	20.005	0.0146569	0.274121	293.15	293.15	0	322.719	322.719	0.0730176	0.072982

723	48.76	8.93177	20.0071	0.0120869	0.264454	293.15	293.15	0	322.552	322.552	0.072998	0.0729634

724	48.68	7.53038	20.0008	0.0101907	0.254976	293.15	293.15	0	322.379	322.379	0.0729769	0.0729434

725	48.58	6.6069	20.0008	0.00894122	0.243823	293.15	293.15	0	322.208	322.208	0.0729555	0.0729215

726	48.48	6.07175	20.0008	0.00821726	0.234753	293.15	293.15	0	322.051	322.051	0.0729309	0.0728975

727	48.37	5.79673	20.0008	0.0078453	0.218112	293.15	293.15	0	321.885	321.885	0.0729067	0.0728726

728	48.26	5.73155	20.0008	0.00775735	0.205881	293.15	293.15	0	321.715	321.715	0.0728806	0.0728461

729	48.14	5.8666	20.0008	0.00794044	0.19454	293.15	293.15	0	321.548	321.548	0.0728529	0.0728167

730	48	6.12605	20.0008	0.00829196	0.184822	293.15	293.15	0	321.375	321.375	0.0728218	0.0727848

731	47.86	6.45076	20.0008	0.00873183	0.176612	293.15	293.15	0	321.211	321.211	0.0727895	0.0727521

732	47.72	6.80249	20.0008	0.00920833	0.166815	293.15	293.15	0	321.051	321.051	0.0727574	0.0727194

733	47.58	7.15774	20.0008	0.00968965	0.158504	293.15	293.15	0	320.881	320.881	0.0727242	0.0726854

734	47.43	7.51943	20.0008	0.0101797	0.152149	293.15	293.15	0	320.713	320.713	0.0726894	0.0726501

735	47.28	7.93538	20.0008	0.0107433	0.142578	293.15	293.15	0	320.544	320.544	0.0726543	0.072614

736	47.11	8.3557	20.0008	0.011313	0.138902	293.15	293.15	0	320.37	320.37	0.0726172	0.072576

737	46.95	8.70419	20.0019	0.0117854	0.136032	293.15	293.15	0	320.223	320.223	0.0725789	0.072538

738	46.8	8.94221	20.005	0.0121082	0.128709	293.15	293.15	0	320.057	320.057	0.0725435	0.0725021

739	46.63	9.16074	19.9946	0.0124047	0.122433	293.15	293.15	0	319.886	319.886	0.0725051	0.0724625

740	46.47	9.38036	19.9914	0.0127028	0.118197	293.15	293.15	0	319.713	319.713	0.0724665	0.0724233

741	46.3	9.58332	19.9946	0.0129783	0.115455	293.15	293.15	0	319.549	319.549	0.0724279	0.072385

742	46.14	9.73946	20.0029	0.0131904	0.109611	293.15	293.15	0	319.383	319.383	0.0723894	0.0723458

743	45.97	9.90854	20.0112	0.01342	0.104241	293.15	293.15	0	319.219	319.219	0.0723507	0.0723072

744	45.8	10.064	20.0008	0.0136313	0.101824	293.15	293.15	0	319.055	319.055	0.0723116	0.0722677

745	45.64	10.1958	20.0008	0.0138104	0.099058	293.15	293.15	0	318.882	318.882	0.0722732	0.0722294

746	45.47	10.2876	20.0008	0.0139356	0.0990735	293.15	293.15	0	318.708	318.708	0.0722329	0.0721889

747	45.3	10.4196	19.9956	0.0141152	0.0934767	293.15	293.15	0	318.544	318.544	0.0721941	0.0721485

748	45.13	10.5267	19.9946	0.0142609	0.0882444	293.15	293.15	0	318.377	318.377	0.0721551	0.0721093

749	44.96	10.5507	20.0008	0.0142942	0.0890678	293.15	293.15	0	318.223	318.223	0.0721153	0.0720696

750	44.8	10.5201	20.0008	0.0142534	0.0875628	293.15	293.15	0	318.052	318.052	0.0720758	0.0720311

751	44.63	10.4604	19.9966	0.0141732	0.0816906	293.15	293.15	0	317.886	317.886	0.0720368	0.0719915

752	44.46	10.369	19.9946	0.0140501	0.0808989	293.15	293.15	0	317.705	317.705	0.0719968	0.0719516

753	44.3	10.2797	20.0008	0.0139298	0.078689	293.15	293.15	0	317.54	317.54	0.0719574	0.0719129

754	44.13	10.261	20.0008	0.0139052	0.0758312	293.15	293.15	0	317.385	317.385	0.0719189	0.0718736

755	43.97	10.3081	20.0008	0.0139698	0.0718001	293.15	293.15	0	317.219	317.219	0.0718802	0.0718347

756	43.8	10.3709	20.0008	0.0140555	0.0682101	293.15	293.15	0	317.049	317.049	0.0718405	0.0717949

757	43.63	10.4412	20.0008	0.0141516	0.06342	293.15	293.15	0	316.881	316.881	0.0718018	0.0717556

758	43.46	10.5551	20.0008	0.0143066	0.059205	293.15	293.15	0	316.708	316.708	0.0717621	0.071716

759	43.29	10.6645	20.0008	0.0144556	0.0578165	293.15	293.15	0	316.545	316.545	0.0717221	0.0716756

760	43.12	10.6986	20.0008	0.0145027	0.0548641	293.15	293.15	0	316.384	316.384	0.0716828	0.0716358

761	42.95	10.7236	20.0008	0.0145373	0.0515239	293.15	293.15	0	316.223	316.223	0.0716435	0.071596

762	42.78	10.7543	20.0008	0.0145797	0.0518725	293.15	293.15	0	316.05	316.05	0.0716036	0.0715559

763	42.62	10.8077	20.0008	0.0146528	0.045193	293.15	293.15	0	315.883	315.883	0.0715645	0.0715165

764	42.45	10.7665	20.0008	0.0145976	0.0449175	293.15	293.15	0	315.713	315.713	0.0715247	0.071477

765	42.28	10.7035	20.0008	0.014513	0.0434003	293.15	293.15	0	315.54	315.54	0.0714856	0.0714378

766	42.12	10.6802	20.0008	0.0144822	0.0397564	293.15	293.15	0	315.381	315.381	0.0714465	0.0713985

767	41.94	10.7303	20.0019	0.0145508	0.0357797	293.15	293.15	0	315.219	315.219	0.0714069	0.0713581

768	41.78	10.8006	20.0102	0.014647	0.0343901	293.15	293.15	0	315.046	315.046	0.0713674	0.0713196

769	41.61	10.8707	20.0008	0.0147428	0.0304386	293.15	293.15	0	314.882	314.882	0.0713283	0.0712794

770	41.44	10.9026	20.0008	0.0147868	0.0299735	293.15	293.15	0	314.715	314.715	0.0712878	0.0712393

771	41.27	10.9285	20.0008	0.0148227	0.0255206	293.15	293.15	0	314.545	314.545	0.0712488	0.0711998

772	41.1	10.9275	20.0008	0.0148221	0.0241004	293.15	293.15	0	314.379	314.379	0.0712085	0.0711589

773	40.93	10.8965	20.0008	0.0147808	0.0226337	293.15	293.15	0	314.224	314.224	0.0711691	0.07112

774	40.76	10.8521	20.0008	0.0147213	0.0227425	293.15	293.15	0	314.041	314.041	0.0711293	0.0710796

775	40.59	10.8758	20.0008	0.0147543	0.0233043	293.15	293.15	0	313.885	313.885	0.0710895	0.0710396

776	40.43	10.9188	20.0008	0.0148134	0.0182776	293.15	293.15	0	313.713	313.713	0.07105	0.0709997

777	40.26	10.9297	19.9966	0.0148288	0.0149678	293.15	293.15	0	313.548	313.548	0.0710112	0.0709607

778	40.09	10.9088	19.9946	0.0148013	0.0161481	293.15	293.15	0	313.384	313.384	0.070971	0.0709206

779	39.92	10.9021	20.0008	0.0147929	0.0118258	293.15	293.15	0	313.21	313.21	0.0709319	0.0708807

780	39.76	10.8889	20.0008	0.0147757	0.0100735	293.15	293.15	0	313.048	313.048	0.0708929	0.0708425

781	39.6	10.8951	20.0008	0.0147849	0.00590254	293.15	293.15	0	312.89	312.89	0.0708551	0.0708042

782	39.43	10.9007	20.0008	0.0147932	-0.00207747	293.15	293.15	0	312.71	312.71	0.0708171	0.0707659

783	39.28	10.87	20.0008	0.0147522	-0.00807696	293.15	293.15	0	312.543	312.543	0.0707797	0.0707288

784	39.12	10.764	20.0008	0.014609	-0.0164328	293.15	293.15	0	312.379	312.379	0.0707427	0.0706924

785	38.97	10.6018	20.0008	0.0143896	-0.0268962	293.15	293.15	0	312.205	312.205	0.0707069	0.0706565

786	38.81	10.4538	20.0008	0.0141894	-0.0363621	293.15	293.15	0	312.045	312.045	0.0706703	0.0706193

787	38.67	10.3193	20.0008	0.0140074	-0.0474883	293.15	293.15	0	311.885	311.885	0.0706347	0.0705843

788	38.52	10.2015	19.9935	0.0138483	-0.0632578	293.15	293.15	0	311.712	311.712	0.0705998	0.0705488

789	38.37	10.0843	19.9925	0.0136898	-0.0773656	293.15	293.15	0	311.548	311.548	0.0705652	0.0705154

790	38.23	10.0149	19.9987	0.0135961	-0.0943873	293.15	293.15	0	311.38	311.38	0.0705317	0.070482

791	38.09	9.95128	19.9966	0.0135103	-0.115787	293.15	293.15	0	311.218	311.218	0.0704986	0.0704487

792	37.95	9.84255	19.9998	0.0133633	-0.137079	293.15	293.15	0	311.052	311.052	0.0704661	0.0704156

793	37.81	9.70892	19.9904	0.0131824	-0.162303	293.15	293.15	0	310.88	310.88	0.0704337	0.070383

794	37.68	9.51488	19.9966	0.0129195	-0.188104	293.15	293.15	0	310.717	310.717	0.0704022	0.0703516

795	37.55	9.32477	20.0008	0.0126618	-0.219662	293.15	293.15	0	310.543	310.543	0.0703715	0.070321

796	37.42	9.21136	20.0008	0.0125083	-0.250193	293.15	293.15	0	310.377	310.377	0.0703401	0.0702901

797	37.29	9.15277	20.0008	0.0124293	-0.28498	293.15	293.15	0	310.206	310.206	0.0703092	0.0702591

798	37.16	9.04893	20.0008	0.0122887	-0.318797	293.15	293.15	0	310.04	310.04	0.0702793	0.0702293

799	37.04	8.87013	20.0008	0.0120464	-0.356025	293.15	293.15	0	309.885	309.885	0.0702491	0.0701996

800	36.91	8.70352	20.0008	0.0118205	-0.39803	293.15	293.15	0	309.722	309.722	0.0702209	0.0701707

801	36.79	8.57762	20.0008	0.01165	-0.440478	293.15	293.15	0	309.547	309.547	0.0701909	0.070142

802	36.67	8.49481	20.006	0.0115379	-0.488006	293.15	293.15	0	309.375	309.375	0.0701624	0.0701127

803	36.55	8.38841	20.006	0.0113938	-0.539523	293.15	293.15	0	309.21	309.21	0.0701346	0.0700844

804	36.43	8.25245	20.0008	0.0112096	-0.589511	293.15	293.15	0	309.044	309.044	0.0701065	0.0700559

805	36.32	8.14416	20.0008	0.0110629	-0.640081	293.15	293.15	0	308.89	308.89	0.0700793	0.0700292

806	36.2	8.01155	20.0008	0.0108831	-0.699113	293.15	293.15	0	308.719	308.719	0.0700521	0.0700025

807	36.09	7.83899	20.0008	0.0106491	-0.762348	293.15	293.15	0	308.552	308.552	0.0700267	0.0699767

808	35.99	7.68248	20.0008	0.0104368	-0.83282	293.15	293.15	0	308.371	308.371	0.0700008	0.0699513

809	35.88	7.58873	20.0008	0.0103098	-0.899225	293.15	293.15	0	308.206	308.206	0.0699746	0.0699253

810	35.77	7.5916	20.0008	0.010314	-0.964953	293.15	293.15	0	308.051	308.051	0.0699491	0.0698995

811	35.66	7.55	20.0008	0.0102578	-1.03917	293.15	293.15	0	307.885	307.885	0.0699239	0.0698746

812	35.56	7.42163	20.0008	0.0100837	-1.11912	293.15	293.15	0	307.716	307.716	0.0698991	0.0698496

813	35.45	7.31204	20.0008	0.00993515	-1.20037	293.15	293.15	0	307.548	307.548	0.0698743	0.0698254

814	35.35	7.15782	19.9977	0.0097259	-1.28865	293.15	293.15	0	307.375	307.375	0.0698505	0.0698016

815	35.25	7.00506	19.9904	0.00951863	-1.37575	293.15	293.15	0	307.211	307.211	0.0698265	0.0697773

816	35.15	6.90788	19.9987	0.00938687	-1.46365	293.15	293.15	0	307.05	307.05	0.069803	0.0697542

817	35.05	6.89665	20.0008	0.00937189	-1.55609	293.15	293.15	0	306.89	306.89	0.0697798	0.0697305

818	34.96	6.88658	20.0008	0.00935846	-1.66063	293.15	293.15	0	306.713	306.713	0.0697576	0.0697085

819	34.86	6.81077	20.0008	0.00925573	-1.76658	293.15	293.15	0	306.544	306.544	0.0697345	0.0696859

820	34.77	6.74364	20.0008	0.00916475	-1.87243	293.15	293.15	0	306.38	306.38	0.069713	0.069664

821	34.68	6.62198	20.0008	0.00899967	-1.97626	293.15	293.15	0	306.223	306.223	0.0696912	0.0696425

822	34.59	6.51306	20.0008	0.00885187	-2.08973	293.15	293.15	0	306.057	306.057	0.0696693	0.0696211

823	34.5	6.44364	20.0008	0.00875777	-2.21326	293.15	293.15	0	305.885	305.885	0.0696487	0.0695995

824	34.41	6.40898	19.9998	0.0087109	-2.34257	293.15	293.15	0	305.713	305.713	0.0696281	0.0695788

825	34.33	6.42071	19.9966	0.00872707	-2.46991	293.15	293.15	0	305.546	305.546	0.0696082	0.0695585

826	34.24	6.4048	20.0008	0.00870568	-2.59722	293.15	293.15	0	305.384	305.384	0.0695876	0.0695376

827	34.15	6.31268	20.0008	0.00858069	-2.73241	293.15	293.15	0	305.219	305.219	0.0695669	0.0695175

828	34.07	6.22116	20.0008	0.0084565	-2.87901	293.15	293.15	0	305.046	305.046	0.069548	0.0694985

829	33.99	6.16511	20.0008	0.00838052	-3.0206	293.15	293.15	0	304.88	304.88	0.0695281	0.0694785

830	33.91	6.04075	19.9966	0.00821168	-3.17214	293.15	293.15	0	304.708	304.708	0.0695082	0.0694595

831	33.83	5.89331	19.9904	0.00801144	-3.32522	293.15	293.15	0	304.542	304.542	0.06949	0.0694409

832	33.75	5.79145	19.9904	0.00787316	-3.48203	293.15	293.15	0	304.378	304.378	0.0694711	0.0694219

833	33.67	5.73329	19.9904	0.00779429	-3.63368	293.15	293.15	0	304.221	304.221	0.0694531	0.0694038

834	33.59	5.74207	19.9935	0.00780641	-3.80253	293.15	293.15	0	304.051	304.051	0.0694348	0.069385

835	33.52	5.74171	20.0008	0.0078061	-3.97379	293.15	293.15	0	303.884	303.884	0.0694164	0.0693673

836	33.44	5.73795	20.0008	0.00780116	-4.14357	293.15	293.15	0	303.723	303.723	0.0693987	0.0693495

837	33.37	5.68727	20.0008	0.00773243	-4.32861	293.15	293.15	0	303.554	303.554	0.0693824	0.0693329

838	33.3	5.60803	20.0008	0.00762486	-4.52004	293.15	293.15	0	303.381	303.381	0.0693652	0.0693159

839	33.23	5.48915	20.0008	0.00746338	-23.7448	293.15	293.15	0	242.591	242.591	0.0693476	0.0692987
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RT54-0.1 GNP-0.1 MWCNT.txt
# Name: RT54-0.1 GNP-0.1 MWCNT

# Date: Tue May 21 16:58:35 2024

# Weight: 9.9 mg

Time(s)	Temperature(°C)	Heat flow(mW)	Gas 1(sccm/min)	DSC_RAW(µV)	POWER(%)	TEMP_CJR_FURNACE(K)	TEMP_CJR_SAMPLE(K)	TEMP_FURNACE(K)	TEMP_NOM_FURNACE(K)	TEMP_NOM_SAMPLE(K)	VOLTAGE_REFERENCE(V)	VOLTAGE_SAMPLE(V)

0	29.92	0.505634	19.9987	0.000688187	0.0642047	293.15	293.15	0	303.253	303.253	0.0685585	0.0685147

1	29.94	1.5049	20.0008	0.00204821	0.121669	293.15	293.15	0	303.426	303.426	0.0685657	0.0685201

2	30.02	2.14098	20.0008	0.00291386	0.164504	293.15	293.15	0	303.596	303.596	0.0685835	0.0685393

3	30.15	2.13841	20.0008	0.00291025	0.19656	293.15	293.15	0	303.764	303.764	0.0686107	0.0685689

4	30.3	1.55938	19.9987	0.00212212	0.217437	293.15	293.15	0	303.933	303.933	0.068645	0.0686049

5	30.47	0.599473	19.9904	0.000815768	0.231437	293.15	293.15	0	304.094	304.094	0.0686828	0.0686449

6	30.64	-0.505784	19.9904	-0.000688239	0.243395	293.15	293.15	0	304.27	304.27	0.0687229	0.0686864

7	30.83	-1.58579	19.9966	-0.00215771	0.25017	293.15	293.15	0	304.423	304.423	0.0687658	0.0687304

8	31.01	-2.55756	20.0008	-0.00347978	0.259111	293.15	293.15	0	304.588	304.588	0.0688081	0.0687737

9	31.2	-3.47555	20.0008	-0.00472849	0.261456	293.15	293.15	0	304.761	304.761	0.0688522	0.0688192

10	31.39	-4.23397	20.0008	-0.00576	0.263169	293.15	293.15	0	304.927	304.927	0.068896	0.0688639

11	31.57	-4.70804	20.0008	-0.00640457	0.268843	293.15	293.15	0	305.099	305.099	0.0689395	0.0689073

12	31.76	-5.08517	20.0008	-0.00691721	0.268433	293.15	293.15	0	305.264	305.264	0.0689843	0.0689523

13	31.95	-5.3787	20.0008	-0.00731607	0.267313	293.15	293.15	0	305.428	305.428	0.0690277	0.0689968

14	32.13	-5.58199	20.0008	-0.00759215	0.268074	293.15	293.15	0	305.601	305.601	0.0690706	0.0690399

15	32.31	-5.74545	19.9914	-0.00781406	0.27226	293.15	293.15	0	305.758	305.758	0.0691121	0.0690815

16	32.49	-5.86885	19.9998	-0.00798145	0.275876	293.15	293.15	0	305.929	305.929	0.0691546	0.069124

17	32.67	-5.91998	20.0008	-0.00805054	0.277654	293.15	293.15	0	306.095	306.095	0.0691962	0.0691661

18	32.84	-5.8557	20.0008	-0.0079627	0.280192	293.15	293.15	0	306.267	306.267	0.0692376	0.0692079

19	33.02	-5.79633	20.0008	-0.00788155	0.279069	293.15	293.15	0	306.426	306.426	0.0692799	0.0692494

20	33.19	-5.73855	20.0008	-0.00780258	0.282797	293.15	293.15	0	306.598	306.598	0.0693203	0.0692904

21	33.37	-5.69398	20.0008	-0.00774155	0.283634	293.15	293.15	0	306.768	306.768	0.069362	0.069332

22	33.54	-5.65349	20.0008	-0.00768611	0.285945	293.15	293.15	0	306.926	306.926	0.0694017	0.0693719

23	33.71	-5.62323	20.0008	-0.00764457	0.290064	293.15	293.15	0	307.096	307.096	0.069442	0.0694121

24	33.88	-5.54172	20.0008	-0.00753337	0.293428	293.15	293.15	0	307.266	307.266	0.0694829	0.0694527

25	34.05	-5.46384	20.0008	-0.00742711	0.29723	293.15	293.15	0	307.423	307.423	0.0695229	0.0694937

26	34.22	-5.42051	20.0008	-0.00736783	0.299648	293.15	293.15	0	307.588	307.588	0.0695618	0.0695331

27	34.39	-5.38708	20.0008	-0.00732201	0.300056	293.15	293.15	0	307.76	307.76	0.0696025	0.0695736

28	34.55	-5.35132	20.0008	-0.00727304	0.301398	293.15	293.15	0	307.934	307.934	0.0696424	0.0696126

29	34.73	-5.3117	20.0008	-0.00721881	0.306705	293.15	293.15	0	308.09	308.09	0.069682	0.0696533

30	34.9	-5.252	19.9904	-0.0071373	0.307114	293.15	293.15	0	308.263	308.263	0.0697221	0.0696937

31	35.06	-5.19822	20.0008	-0.00706386	0.309746	293.15	293.15	0	308.427	308.427	0.0697617	0.0697321

32	35.23	-5.16723	20.0008	-0.00702141	0.313387	293.15	293.15	0	308.6	308.6	0.069801	0.0697715

33	35.39	-5.13862	20.0102	-0.00698216	0.317634	293.15	293.15	0	308.756	308.756	0.0698398	0.0698114

34	35.56	-5.12085	20.0019	-0.00695767	0.325236	293.15	293.15	0	308.93	308.93	0.0698785	0.0698502

35	35.73	-5.20021	20.0008	-0.00706513	0.324478	293.15	293.15	0	309.094	309.094	0.0699184	0.0698903

36	35.9	-5.27846	20.0008	-0.00717107	0.328106	293.15	293.15	0	309.267	309.267	0.0699581	0.0699305

37	36.07	-5.37313	20.0008	-0.00729932	0.328712	293.15	293.15	0	309.424	309.424	0.0699982	0.0699704

38	36.23	-5.44626	20.0008	-0.00739829	0.334663	293.15	293.15	0	309.594	309.594	0.0700378	0.0700097

39	36.4	-5.36014	20.0008	-0.00728094	0.337628	293.15	293.15	0	309.762	309.762	0.0700763	0.0700481

40	36.56	-5.25283	19.9956	-0.00713481	0.339528	293.15	293.15	0	309.94	309.94	0.0701157	0.0700874

41	36.73	-5.20634	20.0008	-0.00707129	0.342248	293.15	293.15	0	310.091	310.091	0.0701562	0.070128

42	36.9	-5.2405	20.0008	-0.00711732	0.346801	293.15	293.15	0	310.264	310.264	0.0701958	0.0701675

43	37.07	-5.27465	20.0008	-0.00716333	0.350511	293.15	293.15	0	310.432	310.432	0.0702344	0.0702072

44	37.23	-5.26269	20.0008	-0.00714675	0.354556	293.15	293.15	0	310.592	310.592	0.0702731	0.0702458

45	37.4	-5.28713	20.0008	-0.00717956	0.358628	293.15	293.15	0	310.759	310.759	0.0703116	0.0702859

46	37.57	-5.24379	20.0008	-0.00712034	0.361293	293.15	293.15	0	310.924	310.924	0.0703526	0.0703257

47	37.74	-5.20067	20.0008	-0.00706144	0.364113	293.15	293.15	0	311.105	311.105	0.0703917	0.0703646

48	37.9	-5.19819	20.0008	-0.00705771	0.367669	293.15	293.15	0	311.262	311.262	0.0704302	0.0704042

49	38.07	-5.2073	20.0008	-0.00706972	0.370027	293.15	293.15	0	311.425	311.425	0.0704692	0.0704435

50	38.23	-5.20286	20.0008	-0.00706334	0.37567	293.15	293.15	0	311.599	311.599	0.0705084	0.0704824

51	38.4	-5.23053	20.0008	-0.00710054	0.377962	293.15	293.15	0	311.763	311.763	0.0705484	0.0705225

52	38.57	-5.26558	20.0008	-0.00714774	0.381196	293.15	293.15	0	311.936	311.936	0.0705874	0.0705623

53	38.74	-5.30294	20.0008	-0.00719808	0.380001	293.15	293.15	0	312.091	312.091	0.0706288	0.0706024

54	38.91	-5.36514	20.0008	-0.00728214	0.384767	293.15	293.15	0	312.273	312.273	0.0706677	0.0706423

55	39.08	-5.40824	20.0008	-0.00734027	0.388942	293.15	293.15	0	312.423	312.423	0.0707072	0.0706818

56	39.25	-5.46984	19.9925	-0.00742349	0.393727	293.15	293.15	0	312.596	312.596	0.0707453	0.0707216

57	39.41	-5.49785	19.9987	-0.00746113	0.393025	293.15	293.15	0	312.765	312.765	0.0707859	0.07076

58	39.58	-5.48191	20.0008	-0.00743913	0.399961	293.15	293.15	0	312.933	312.933	0.0708249	0.0707994

59	39.74	-5.43124	20.0008	-0.00736998	0.402089	293.15	293.15	0	313.09	313.09	0.0708643	0.0708388

60	39.91	-5.41734	20.0008	-0.00735075	0.404951	293.15	293.15	0	313.258	313.258	0.0709033	0.0708781

61	40.08	-5.36983	20.0008	-0.00728591	0.40866	293.15	293.15	0	313.427	313.427	0.0709425	0.0709178

62	40.24	-5.31151	20.0008	-0.00720642	0.415464	293.15	293.15	0	313.596	313.596	0.0709805	0.070957

63	40.41	-5.27141	20.0008	-0.00715165	0.416778	293.15	293.15	0	313.757	313.757	0.0710202	0.0709965

64	40.58	-5.28923	20.0008	-0.00717546	0.420949	293.15	293.15	0	313.93	313.93	0.0710597	0.0710353

65	40.75	-5.32554	20.0008	-0.00722435	0.424563	293.15	293.15	0	314.096	314.096	0.0710987	0.0710758

66	40.91	-5.33777	20.0008	-0.00724057	0.42465	293.15	293.15	0	314.269	314.269	0.0711385	0.0711147

67	41.08	-5.35463	20.0008	-0.00726306	0.431578	293.15	293.15	0	314.424	314.424	0.0711781	0.0711548

68	41.25	-5.35518	20.0008	-0.00726344	0.431691	293.15	293.15	0	314.597	314.597	0.0712182	0.0711944

69	41.42	-5.39709	19.9904	-0.0073199	0.435172	293.15	293.15	0	314.761	314.761	0.0712569	0.0712344

70	41.58	-5.46748	20.0008	-0.007415	0.4402	293.15	293.15	0	314.926	314.926	0.0712955	0.0712734

71	41.75	-5.45938	19.9914	-0.00740364	0.441152	293.15	293.15	0	315.093	315.093	0.0713351	0.0713127

72	41.92	-5.41384	19.9998	-0.0073415	0.447464	293.15	293.15	0	315.262	315.262	0.0713742	0.0713525

73	42.08	-5.35718	20.0008	-0.00726431	0.450069	293.15	293.15	0	315.429	315.429	0.0714134	0.0713908

74	42.25	-5.3241	20.0008	-0.00721909	0.454068	293.15	293.15	0	315.6	315.6	0.0714528	0.0714306

75	42.42	-5.3421	20.0008	-0.00724312	0.455714	293.15	293.15	0	315.759	315.759	0.0714924	0.0714704

76	42.59	-5.39747	20.0008	-0.00731782	0.46058	293.15	293.15	0	315.938	315.938	0.0715311	0.0715095

77	42.76	-5.437	20.0008	-0.00737103	0.462981	293.15	293.15	0	316.088	316.088	0.0715711	0.0715495

78	42.92	-5.41289	20.0008	-0.00733798	0.466153	293.15	293.15	0	316.262	316.262	0.0716106	0.0715887

79	43.09	-5.39381	20.0008	-0.00731174	0.469091	293.15	293.15	0	316.426	316.426	0.0716495	0.071628

80	43.26	-5.36266	20.0008	-0.00726914	0.475002	293.15	293.15	0	316.594	316.594	0.0716892	0.0716681

81	43.42	-5.3433	20.0008	-0.00724255	0.480379	293.15	293.15	0	316.756	316.756	0.0717276	0.0717054

82	43.58	-5.3063	20.0008	-0.00719202	0.482627	293.15	293.15	0	316.922	316.922	0.0717665	0.0717448

83	43.76	-5.29479	20.0008	-0.00717605	0.483849	293.15	293.15	0	317.093	317.093	0.0718066	0.0717853

84	43.92	-5.32933	20.0008	-0.00722251	0.487547	293.15	293.15	0	317.267	317.267	0.0718454	0.071824

85	44.09	-5.32702	20.0008	-0.007219	0.492349	293.15	293.15	0	317.423	317.423	0.0718849	0.071864

86	44.26	-5.34848	20.0008	-0.00724771	0.493828	293.15	293.15	0	317.596	317.596	0.0719242	0.0719039

87	44.43	-5.39127	19.9904	-0.00730531	0.497102	293.15	293.15	0	317.76	317.76	0.0719632	0.0719439

88	44.6	-5.42062	19.9956	-0.00734471	0.501688	293.15	293.15	0	317.943	317.943	0.0720031	0.0719832

89	44.77	-5.42214	20.0008	-0.00734639	0.502995	293.15	293.15	0	318.091	318.091	0.0720426	0.072023

90	44.93	-5.4	20.0008	-0.00731603	0.506076	293.15	293.15	0	318.263	318.263	0.0720827	0.0720624

91	45.09	-5.39769	20.0008	-0.00731254	0.510448	293.15	293.15	0	318.434	318.434	0.0721211	0.0721005

92	45.26	-5.40229	20.0008	-0.00731839	0.513327	293.15	293.15	0	318.607	318.607	0.0721599	0.0721398

93	45.43	-5.38665	20.0008	-0.00729683	0.521208	293.15	293.15	0	318.766	318.766	0.072198	0.0721791

94	45.59	-5.38379	20.0008	-0.0072926	0.522746	293.15	293.15	0	318.94	318.94	0.0722377	0.0722184

95	45.77	-5.44433	20.0008	-0.00737421	0.523777	293.15	293.15	0	319.087	319.087	0.0722776	0.0722589

96	45.94	-5.5303	19.9956	-0.00749027	0.527167	293.15	293.15	0	319.255	319.255	0.0723167	0.0722985

97	46.1	-5.55281	20.0008	-0.00752038	0.531389	293.15	293.15	0	319.425	319.425	0.0723559	0.0723373

98	46.27	-5.51165	20.0008	-0.00746426	0.535855	293.15	293.15	0	319.601	319.601	0.0723958	0.0723776

99	46.43	-5.50009	20.0008	-0.00744823	0.539722	293.15	293.15	0	319.754	319.754	0.0724347	0.0724162

100	46.6	-5.49737	20.0008	-0.00744418	0.542046	293.15	293.15	0	319.929	319.929	0.0724731	0.0724544

101	46.77	-5.48832	19.9998	-0.00743153	0.544931	293.15	293.15	0	320.1	320.1	0.0725129	0.0724945

102	46.93	-5.51124	19.9914	-0.00746219	0.552407	293.15	293.15	0	320.274	320.274	0.072551	0.0725333

103	47.1	-5.47715	20.0008	-0.00741566	0.553083	293.15	293.15	0	320.421	320.421	0.0725912	0.0725728

104	47.27	-5.41717	20.0008	-0.00733407	0.556563	293.15	293.15	0	320.595	320.595	0.0726299	0.0726118

105	47.43	-5.40975	20.0008	-0.00732366	0.559622	293.15	293.15	0	320.768	320.768	0.0726684	0.0726511

106	47.6	-5.42421	20.0008	-0.00734287	0.565207	293.15	293.15	0	320.924	320.924	0.072707	0.0726899

107	47.77	-5.43654	20.0008	-0.00735918	0.567581	293.15	293.15	0	321.089	321.089	0.0727472	0.0727307

108	47.94	-5.43983	20.0008	-0.00736326	0.571052	293.15	293.15	0	321.26	321.26	0.0727868	0.0727699

109	48.11	-5.44814	20.0008	-0.00737413	0.573814	293.15	293.15	0	321.426	321.426	0.0728259	0.0728093

110	48.27	-5.47355	20.0008	-0.00740815	0.581464	293.15	293.15	0	321.597	321.597	0.0728648	0.0728482

111	48.44	-5.51996	20.0008	-0.00747058	0.584976	293.15	293.15	0	321.756	321.756	0.0729037	0.0728875

112	48.61	-5.59608	19.9925	-0.0075732	0.586707	293.15	293.15	0	321.934	321.934	0.0729426	0.0729278

113	48.78	-5.64696	19.9977	-0.00764167	0.587388	293.15	293.15	0	322.086	322.086	0.0729832	0.0729669

114	48.94	-5.63962	20.0008	-0.00763136	0.592803	293.15	293.15	0	322.263	322.263	0.0730221	0.0730063

115	49.11	-5.56858	19.9987	-0.00753485	0.597804	293.15	293.15	0	322.433	322.433	0.0730615	0.073046

116	49.28	-5.50681	19.9914	-0.00745088	0.601533	293.15	293.15	0	322.599	322.599	0.0731008	0.073085

117	49.44	-5.47929	20.0008	-0.00741328	0.604661	293.15	293.15	0	322.762	322.762	0.0731392	0.0731241

118	49.61	-5.46549	20.0008	-0.00739423	0.607821	293.15	293.15	0	322.935	322.935	0.0731781	0.0731632

119	49.78	-5.44904	20.0008	-0.0073716	0.61062	293.15	293.15	0	323.1	323.1	0.073217	0.0732023

120	49.95	-5.43834	20.0008	-0.00735674	0.614648	293.15	293.15	0	323.256	323.256	0.0732571	0.073243

121	50.11	-5.42873	19.9956	-0.00734338	0.619852	293.15	293.15	0	323.421	323.421	0.0732957	0.0732814

122	50.28	-5.41861	19.9904	-0.00732932	0.62063	293.15	293.15	0	323.593	323.593	0.0733354	0.0733207

123	50.45	-5.44243	20.0008	-0.00736115	0.625999	293.15	293.15	0	323.766	323.766	0.0733749	0.07336

124	50.61	-5.45844	20.0008	-0.00738244	0.63026	293.15	293.15	0	323.931	323.931	0.0734135	0.073399

125	50.79	-5.47436	20.0008	-0.00740359	0.632509	293.15	293.15	0	324.096	324.096	0.0734532	0.0734394

126	50.95	-5.47015	20.0008	-0.00739752	0.637369	293.15	293.15	0	324.268	324.268	0.0734917	0.0734779

127	51.12	-5.456	20.0008	-0.00737802	0.639703	293.15	293.15	0	324.426	324.426	0.0735304	0.0735168

128	51.29	-5.48301	20.0008	-0.00741414	0.640167	293.15	293.15	0	324.597	324.597	0.0735708	0.0735576

129	51.45	-5.53611	20.0008	-0.00748558	0.649263	293.15	293.15	0	324.764	324.764	0.0736086	0.0735953

130	51.62	-5.54764	20.0008	-0.00750079	0.652886	293.15	293.15	0	324.937	324.937	0.0736466	0.0736347

131	51.78	-5.5208	20.0008	-0.00746412	0.656009	293.15	293.15	0	325.089	325.089	0.0736862	0.0736741

132	51.95	-5.49548	19.9956	-0.00742952	0.658905	293.15	293.15	0	325.258	325.258	0.073726	0.0737126

133	52.12	-5.55698	20.0008	-0.00751227	0.665014	293.15	293.15	0	325.431	325.431	0.0737652	0.0737532

134	52.29	-5.59468	20.0008	-0.00756286	0.667409	293.15	293.15	0	325.59	325.59	0.0738042	0.0737926

135	52.46	-5.58121	20.0008	-0.00754426	0.670832	293.15	293.15	0	325.752	325.752	0.0738439	0.0738324

136	52.62	-5.5668	20.0008	-0.0075244	0.67229	293.15	293.15	0	325.927	325.927	0.0738831	0.0738713

137	52.8	-5.54997	20.0008	-0.00750125	0.678235	293.15	293.15	0	326.098	326.098	0.0739223	0.0739117

138	52.96	-5.50585	20.0008	-0.00744125	0.68102	293.15	293.15	0	326.271	326.271	0.0739611	0.0739498

139	53.13	-5.48732	20.0008	-0.00741583	0.68434	293.15	293.15	0	326.42	326.42	0.0740007	0.0739897

140	53.29	-5.53809	20.0008	-0.00748407	0.686569	293.15	293.15	0	326.601	326.601	0.0740386	0.074028

141	53.46	-5.57816	20.0008	-0.00753784	0.694851	293.15	293.15	0	326.765	326.765	0.0740785	0.0740674

142	53.63	-5.58498	20.0008	-0.00754667	0.697184	293.15	293.15	0	326.931	326.931	0.0741167	0.0741071

143	53.8	-5.59421	20.0008	-0.00755876	0.699002	293.15	293.15	0	327.093	327.093	0.0741563	0.0741462

144	53.96	-5.58519	20.0008	-0.00754619	0.702896	293.15	293.15	0	327.259	327.259	0.0741954	0.0741853

145	54.13	-5.55525	20.0008	-0.00750536	0.709131	293.15	293.15	0	327.432	327.432	0.0742344	0.0742253

146	54.3	-5.48963	20.0008	-0.00741633	0.713806	293.15	293.15	0	327.595	327.595	0.0742735	0.0742636

147	54.46	-5.50348	20.0008	-0.00743467	0.716411	293.15	293.15	0	327.754	327.754	0.0743128	0.0743026

148	54.63	-5.52801	19.9925	-0.00746743	0.718105	293.15	293.15	0	327.933	327.933	0.074352	0.0743414

149	54.8	-5.52263	19.9935	-0.00745978	0.721881	293.15	293.15	0	328.101	328.101	0.0743906	0.0743808

150	54.96	-5.57052	20.0008	-0.00752409	0.729357	293.15	293.15	0	328.27	328.27	0.0744297	0.0744203

151	55.13	-5.66462	20.0008	-0.00765079	0.733298	293.15	293.15	0	328.429	328.429	0.0744676	0.0744594

152	55.3	-5.72261	20.0008	-0.00772872	0.736873	293.15	293.15	0	328.603	328.603	0.0745075	0.0744992

153	55.46	-5.77561	20.0008	-0.00779991	0.741026	293.15	293.15	0	328.767	328.767	0.0745463	0.0745376

154	55.63	-5.84051	20.0008	-0.00788716	0.745129	293.15	293.15	0	328.925	328.925	0.0745853	0.0745772

155	55.8	-5.90404	20.0008	-0.00797254	0.748204	293.15	293.15	0	329.097	329.097	0.0746249	0.0746168

156	55.97	-5.94186	20.0008	-0.0080232	0.748949	293.15	293.15	0	329.263	329.263	0.0746649	0.0746568

157	56.14	-5.98531	20.0008	-0.00808145	0.74973	293.15	293.15	0	329.426	329.426	0.0747049	0.0746959

158	56.3	-5.95677	20.0008	-0.00804252	0.75927	293.15	293.15	0	329.591	329.591	0.0747427	0.0747344

159	56.47	-5.96966	20.0008	-0.00805952	0.761051	293.15	293.15	0	329.755	329.755	0.0747817	0.0747727

160	56.63	-6.03121	20.0008	-0.00814222	0.765538	293.15	293.15	0	329.93	329.93	0.0748199	0.0748112

161	56.8	-6.08679	20.0008	-0.00821684	0.770976	293.15	293.15	0	330.094	330.094	0.0748582	0.0748506

162	56.97	-6.18575	20.0008	-0.00835	0.774541	293.15	293.15	0	330.265	330.265	0.0748971	0.0748896

163	57.13	-6.27166	20.0008	-0.00846554	0.780547	293.15	293.15	0	330.431	330.431	0.0749362	0.0749292

164	57.3	-6.33222	20.0008	-0.00854685	0.785516	293.15	293.15	0	330.602	330.602	0.0749753	0.0749678

165	57.47	-6.49694	20.0008	-0.00876874	0.789143	293.15	293.15	0	330.762	330.762	0.0750139	0.0750071

166	57.63	-6.74229	20.0008	-0.00909943	0.795812	293.15	293.15	0	330.934	330.934	0.0750519	0.0750456

167	57.8	-6.98823	20.0008	-0.00943086	0.800838	293.15	293.15	0	331.099	331.099	0.0750911	0.0750855

168	57.96	-7.27051	20.0029	-0.00981133	0.804414	293.15	293.15	0	331.259	331.259	0.0751295	0.0751235

169	58.13	-7.58503	20.0091	-0.0102352	0.812143	293.15	293.15	0	331.428	331.428	0.075167	0.0751623

170	58.3	-7.94004	20.0008	-0.0107137	0.818532	293.15	293.15	0	331.596	331.596	0.075205	0.075202

171	58.46	-8.40147	20.0008	-0.0113358	0.826695	293.15	293.15	0	331.749	331.749	0.0752426	0.0752398

172	58.63	-9.01556	20.0008	-0.0121637	0.834539	293.15	293.15	0	331.924	331.924	0.0752811	0.0752807

173	58.8	-9.79979	20.0008	-0.0132212	0.844902	293.15	293.15	0	332.096	332.096	0.075317	0.0753192

174	58.97	-10.8331	19.9956	-0.0146145	0.853753	293.15	293.15	0	332.269	332.269	0.0753545	0.0753581

175	59.13	-12.1392	20.0008	-0.0163757	0.862436	293.15	293.15	0	332.417	332.417	0.0753907	0.0753974

176	59.29	-13.7482	20.0008	-0.0185453	0.878879	293.15	293.15	0	332.599	332.599	0.0754266	0.0754351

177	59.45	-15.5642	20.0008	-0.0209939	0.894422	293.15	293.15	0	332.763	332.763	0.0754606	0.0754724

178	59.61	-17.6692	20.0008	-0.0238321	0.91514	293.15	293.15	0	332.936	332.936	0.0754942	0.0755096

179	59.78	-20.185	20.0008	-0.027224	0.930463	293.15	293.15	0	333.093	333.093	0.0755283	0.0755497

180	59.95	-23.04	20.0008	-0.0310731	0.954742	293.15	293.15	0	333.273	333.273	0.0755624	0.0755881

181	60.11	-26.23	20.0008	-0.0353736	0.975144	293.15	293.15	0	333.422	333.422	0.0755952	0.0756268

182	60.27	-29.6686	20.0008	-0.0400088	0.99646	293.15	293.15	0	333.596	333.596	0.0756288	0.0756646

183	60.45	-33.3368	20.0008	-0.0449531	1.01977	293.15	293.15	0	333.766	333.766	0.0756629	0.075705

184	60.62	-37.0236	20.0008	-0.0499221	1.04263	293.15	293.15	0	333.933	333.933	0.075698	0.0757445

185	60.8	-40.657	20.0008	-0.0548183	1.0591	293.15	293.15	0	334.09	334.09	0.0757354	0.0757869

186	60.97	-44.0937	20.0008	-0.0594488	1.07745	293.15	293.15	0	334.257	334.257	0.0757722	0.0758284

187	61.15	-47.2885	20.0008	-0.0637528	1.09543	293.15	293.15	0	334.427	334.427	0.0758103	0.0758704

188	61.34	-50.2638	20.0008	-0.0677601	1.10902	293.15	293.15	0	334.604	334.604	0.0758512	0.0759149

189	61.53	-52.9913	19.9998	-0.0714329	1.12031	293.15	293.15	0	334.757	334.757	0.0758919	0.0759587

190	61.72	-55.5272	19.9904	-0.0748471	1.13347	293.15	293.15	0	334.93	334.93	0.0759332	0.0760028

191	61.91	-57.6906	19.9966	-0.0777585	1.14033	293.15	293.15	0	335.097	335.097	0.075976	0.0760484

192	62.11	-59.5405	20.0008	-0.0802473	1.14408	293.15	293.15	0	335.269	335.269	0.0760196	0.0760932

193	62.29	-61.0641	20.0008	-0.0822961	1.15416	293.15	293.15	0	335.424	335.424	0.0760623	0.0761371

194	62.48	-62.2404	20.0008	-0.0838767	1.15655	293.15	293.15	0	335.599	335.599	0.0761049	0.0761812

195	62.67	-63.0919	20.0008	-0.0850193	1.16003	293.15	293.15	0	335.761	335.761	0.076149	0.0762254

196	62.86	-63.7185	20.0112	-0.0858587	1.15968	293.15	293.15	0	335.935	335.935	0.0761934	0.0762701

197	63.05	-64.1578	20.0008	-0.0864458	1.16624	293.15	293.15	0	336.099	336.099	0.0762363	0.0763133

198	63.23	-64.3418	19.9904	-0.0866889	1.16734	293.15	293.15	0	336.272	336.272	0.0762796	0.0763564

199	63.42	-64.3257	19.9946	-0.0866623	1.16493	293.15	293.15	0	336.429	336.429	0.0763236	0.0764

200	63.6	-64.1154	20.0008	-0.0863742	1.16293	293.15	293.15	0	336.61	336.61	0.0763676	0.0764426

201	63.78	-63.6779	20.0008	-0.0857801	1.16113	293.15	293.15	0	336.758	336.758	0.0764107	0.0764857

202	63.96	-63.0773	19.9977	-0.0849664	1.16052	293.15	293.15	0	336.933	336.933	0.0764539	0.0765275

203	64.14	-62.3283	19.9904	-0.0839528	1.15926	293.15	293.15	0	337.101	337.101	0.0764957	0.0765693

204	64.32	-61.4903	19.9987	-0.0828197	1.15387	293.15	293.15	0	337.26	337.26	0.0765394	0.0766107

205	64.49	-60.6236	20.0008	-0.0816481	1.15319	293.15	293.15	0	337.429	337.429	0.0765808	0.076651

206	64.66	-59.6574	20.0008	-0.0803426	1.15436	293.15	293.15	0	337.599	337.599	0.0766222	0.0766911

207	64.84	-58.5725	20.0008	-0.0788774	1.15115	293.15	293.15	0	337.756	337.756	0.0766645	0.0767314

208	65.01	-57.3075	19.9998	-0.07717	1.14594	293.15	293.15	0	337.921	337.921	0.0767065	0.0767713

209	65.18	-55.8854	19.9904	-0.075251	1.14209	293.15	293.15	0	338.094	338.094	0.0767476	0.0768112

210	65.35	-54.4125	19.9977	-0.0732641	1.13531	293.15	293.15	0	338.268	338.268	0.0767895	0.0768508

211	65.52	-52.8473	20.0112	-0.0711529	1.13078	293.15	293.15	0	338.423	338.423	0.076832	0.0768905

212	65.69	-51.0758	20.0008	-0.0687643	1.12414	293.15	293.15	0	338.596	338.596	0.0768742	0.0769303

213	65.85	-49.2514	20.0008	-0.0663047	1.11677	293.15	293.15	0	338.769	338.769	0.0769153	0.0769687

214	66.01	-47.3044	20.0008	-0.0636806	1.11212	293.15	293.15	0	338.933	338.933	0.0769557	0.0770058

215	66.18	-44.9717	20.0008	-0.0605372	1.10354	293.15	293.15	0	339.09	339.09	0.0769987	0.0770449

216	66.34	-42.2116	20.0008	-0.0568189	1.09273	293.15	293.15	0	339.271	339.271	0.0770423	0.0770837

217	66.52	-38.9966	20.0008	-0.0524886	1.07717	293.15	293.15	0	339.437	339.437	0.0770872	0.0771237

218	66.69	-35.2925	19.9977	-0.0475006	1.05609	293.15	293.15	0	339.602	339.602	0.0771336	0.0771638

219	66.86	-31.1789	19.9935	-0.0419619	1.03749	293.15	293.15	0	339.763	339.763	0.07718	0.0772041

220	67.02	-27.0227	20.0008	-0.0363665	1.025	293.15	293.15	0	339.931	339.931	0.077223	0.0772419

221	67.18	-22.9805	19.9956	-0.0309251	1.01055	293.15	293.15	0	340.087	340.087	0.0772646	0.0772792

222	67.34	-19.2116	19.9987	-0.025852	0.997287	293.15	293.15	0	340.255	340.255	0.077306	0.0773159

223	67.48	-15.8672	19.9904	-0.0213507	0.991343	293.15	293.15	0	340.433	340.433	0.0773435	0.0773495

224	67.63	-12.9588	19.9977	-0.0174364	0.989611	293.15	293.15	0	340.601	340.601	0.0773791	0.0773833

225	67.77	-10.6432	19.9998	-0.0143201	0.98925	293.15	293.15	0	340.754	340.754	0.0774136	0.0774163

226	67.91	-8.78174	19.9904	-0.0118151	0.99361	293.15	293.15	0	340.928	340.928	0.0774457	0.077448

227	68.05	-7.32686	19.9966	-0.00985723	0.99313	293.15	293.15	0	341.093	341.093	0.0774804	0.0774815

228	68.19	-6.16585	20.0008	-0.00829492	1.00029	293.15	293.15	0	341.265	341.265	0.0775136	0.0775135

229	68.33	-5.25537	20.0008	-0.00706976	1.00442	293.15	293.15	0	341.421	341.421	0.0775467	0.0775459

230	68.47	-4.59554	19.9956	-0.00618186	1.01091	293.15	293.15	0	341.594	341.594	0.0775798	0.0775795

231	68.62	-4.17037	20.0008	-0.00560968	1.01744	293.15	293.15	0	341.768	341.768	0.0776139	0.077614

232	68.76	-3.94421	20.0008	-0.00530522	1.02566	293.15	293.15	0	341.932	341.932	0.0776486	0.077648

233	68.91	-3.74796	20.0008	-0.00504103	1.03254	293.15	293.15	0	342.097	342.097	0.0776831	0.0776829

234	69.06	-3.55172	20.0008	-0.00477686	1.03964	293.15	293.15	0	342.269	342.269	0.0777179	0.0777177

235	69.22	-3.41393	19.9956	-0.00459133	1.04693	293.15	293.15	0	342.436	342.436	0.077754	0.0777535

236	69.37	-3.41764	20.0008	-0.0045961	1.05163	293.15	293.15	0	342.598	342.598	0.0777901	0.0777904

237	69.53	-3.52508	20.0008	-0.00474037	1.05954	293.15	293.15	0	342.756	342.756	0.0778265	0.077827

238	69.69	-3.62848	20.0008	-0.00487918	1.06509	293.15	293.15	0	342.935	342.935	0.0778636	0.0778649

239	69.86	-3.70053	20.0008	-0.00497581	1.06959	293.15	293.15	0	343.086	343.086	0.0779009	0.0779027

240	70.02	-3.71319	20.0008	-0.00499259	1.076	293.15	293.15	0	343.262	343.262	0.0779388	0.0779401

241	70.18	-3.74523	20.0008	-0.00503543	1.08324	293.15	293.15	0	343.432	343.432	0.0779768	0.0779786

242	70.34	-3.7626	20.0008	-0.00505853	1.08878	293.15	293.15	0	343.598	343.598	0.0780149	0.0780166

243	70.51	-3.81225	19.9998	-0.00512503	1.09167	293.15	293.15	0	343.753	343.753	0.0780529	0.0780546

244	70.67	-3.83083	19.9904	-0.00514975	1.09656	293.15	293.15	0	343.919	343.919	0.0780911	0.078093

245	70.84	-3.87431	19.9904	-0.00520794	1.10139	293.15	293.15	0	344.1	344.1	0.0781294	0.0781322

246	71.01	-3.936	19.9914	-0.0052906	1.10866	293.15	293.15	0	344.265	344.265	0.0781674	0.0781709

247	71.17	-3.97863	20.0008	-0.00534763	1.1109	293.15	293.15	0	344.429	344.429	0.0782068	0.0782095

248	71.34	-4.06277	20.0008	-0.00546045	1.11412	293.15	293.15	0	344.594	344.594	0.0782457	0.0782484

249	71.5	-4.13779	20.0008	-0.005561	1.12089	293.15	293.15	0	344.751	344.751	0.078283	0.0782867

250	71.68	-4.17231	20.0008	-0.0056071	1.12288	293.15	293.15	0	344.922	344.922	0.0783237	0.0783269

251	71.84	-4.2003	20.0008	-0.00564444	1.13053	293.15	293.15	0	345.103	345.103	0.078362	0.0783655

252	72.01	-4.26005	20.0008	-0.00572444	1.13471	293.15	293.15	0	345.261	345.261	0.0784004	0.0784044

253	72.18	-4.32825	20.0008	-0.00581579	1.13682	293.15	293.15	0	345.427	345.427	0.0784396	0.0784441

254	72.34	-4.304	20.0008	-0.00578292	1.14105	293.15	293.15	0	345.597	345.597	0.078478	0.0784821

255	72.51	-4.33038	20.0008	-0.00581807	1.14799	293.15	293.15	0	345.764	345.764	0.0785163	0.0785214

256	72.68	-4.36389	20.0008	-0.00586278	1.14887	293.15	293.15	0	345.937	345.937	0.0785565	0.0785611

257	72.85	-4.38416	20.0008	-0.00588972	1.15342	293.15	293.15	0	346.088	346.088	0.0785949	0.0785998

258	73.01	-4.40187	19.9987	-0.00591322	1.15885	293.15	293.15	0	346.258	346.258	0.0786331	0.0786384

259	73.18	-4.3843	19.9904	-0.00588931	1.16314	293.15	293.15	0	346.431	346.431	0.0786734	0.0786783

260	73.35	-4.32852	19.9925	-0.00581409	1.16942	293.15	293.15	0	346.599	346.599	0.0787111	0.0787163

261	73.51	-4.25398	20.0008	-0.00571369	1.17308	293.15	293.15	0	346.752	346.752	0.0787493	0.0787547

262	73.68	-4.25643	20.0008	-0.0057167	1.17681	293.15	293.15	0	346.927	346.927	0.0787887	0.0787933

263	73.85	-4.24402	19.9998	-0.00569973	1.18482	293.15	293.15	0	347.098	347.098	0.0788265	0.0788329

264	74.02	-4.23578	19.9914	-0.00568838	1.18725	293.15	293.15	0	347.271	347.271	0.0788661	0.0788721

265	74.18	-4.22218	20.0008	-0.00566983	1.19018	293.15	293.15	0	347.419	347.419	0.0789048	0.0789109

266	74.35	-4.20729	20.0008	-0.00564955	1.19237	293.15	293.15	0	347.592	347.592	0.0789441	0.0789504

267	74.52	-4.23919	20.0008	-0.0056921	1.1997	293.15	293.15	0	347.756	347.756	0.0789821	0.0789892

268	74.69	-4.24817	20.0008	-0.00570387	1.20604	293.15	293.15	0	347.93	347.93	0.079021	0.0790281

269	74.85	-4.2159	20.0008	-0.00566025	1.20772	293.15	293.15	0	348.093	348.093	0.0790597	0.0790663

270	75.02	-4.18867	20.0008	-0.00562341	1.21105	293.15	293.15	0	348.275	348.275	0.079098	0.0791058

271	75.19	-4.17303	20.005	-0.00560213	1.21441	293.15	293.15	0	348.423	348.423	0.0791385	0.0791451

272	75.35	-4.20644	20.0112	-0.0056467	1.22049	293.15	293.15	0	348.596	348.596	0.0791766	0.0791832

273	75.52	-4.25526	20.0019	-0.00571195	1.22558	293.15	293.15	0	348.768	348.768	0.0792154	0.0792219

274	75.69	-4.25487	20.0008	-0.00571114	1.22756	293.15	293.15	0	348.935	348.935	0.0792539	0.0792607

275	75.85	-4.27488	20.0008	-0.00573771	1.23074	293.15	293.15	0	349.091	349.091	0.0792936	0.0792997

276	76.02	-4.23781	20.0008	-0.00568766	1.23964	293.15	293.15	0	349.266	349.266	0.0793315	0.0793387

277	76.19	-4.12787	20.0008	-0.00553983	1.24371	293.15	293.15	0	349.43	349.43	0.0793698	0.0793775

278	76.35	-4.05062	20.0008	-0.00543589	1.24646	293.15	293.15	0	349.603	349.603	0.0794096	0.0794156

279	76.52	-3.98799	20.0008	-0.00535157	1.25206	293.15	293.15	0	349.75	349.75	0.0794472	0.0794542

280	76.69	-3.93625	20.0008	-0.00528186	1.25873	293.15	293.15	0	349.916	349.916	0.0794859	0.0794941

281	76.86	-3.8839	20.0008	-0.00521136	1.26242	293.15	293.15	0	350.097	350.097	0.0795248	0.0795334

282	77.03	-3.86802	20.0008	-0.00518978	1.26492	293.15	293.15	0	350.262	350.262	0.0795642	0.0795724

283	77.19	-3.85888	20.0008	-0.00517727	1.26719	293.15	293.15	0	350.426	350.426	0.0796026	0.0796106

284	77.36	-3.85435	20.0008	-0.00517092	1.27412	293.15	293.15	0	350.591	350.591	0.0796421	0.0796498

285	77.52	-3.84764	20.0008	-0.00516167	1.27597	293.15	293.15	0	350.766	350.766	0.0796803	0.0796881

286	77.69	-3.84927	20.0008	-0.0051636	1.28018	293.15	293.15	0	350.928	350.928	0.0797191	0.079727

287	77.86	-3.85121	20.0008	-0.00516594	1.28591	293.15	293.15	0	351.094	351.094	0.0797572	0.0797657

288	78.03	-3.80314	20.0008	-0.0051012	1.29041	293.15	293.15	0	351.265	351.265	0.0797962	0.0798046

289	78.19	-3.76422	20.0008	-0.00504874	1.29415	293.15	293.15	0	351.424	351.424	0.0798347	0.079843

290	78.36	-3.73657	20.0008	-0.00501141	1.30217	293.15	293.15	0	351.593	351.593	0.0798729	0.0798824

291	78.53	-3.71417	20.0008	-0.00498111	1.30468	293.15	293.15	0	351.762	351.762	0.0799118	0.0799213

292	78.7	-3.69911	20.0008	-0.00496066	1.30808	293.15	293.15	0	351.935	351.935	0.079951	0.0799608

293	78.86	-3.6609	20.0008	-0.00490917	1.31347	293.15	293.15	0	352.086	352.086	0.0799893	0.0799989

294	79.03	-3.64077	19.9956	-0.00488194	1.31932	293.15	293.15	0	352.256	352.256	0.0800278	0.080038

295	79.2	-3.59577	20.0008	-0.00482135	1.32396	293.15	293.15	0	352.432	352.432	0.0800668	0.0800767

296	79.36	-3.57488	19.9998	-0.0047931	1.32982	293.15	293.15	0	352.592	352.592	0.0801048	0.0801152

297	79.53	-3.5237	19.9904	-0.00472425	1.33237	293.15	293.15	0	352.76	352.76	0.0801436	0.0801536

298	79.7	-3.50497	19.9914	-0.0046989	1.33795	293.15	293.15	0	352.932	352.932	0.080183	0.0801927

299	79.87	-3.60258	20.0008	-0.00482951	1.34092	293.15	293.15	0	353.088	353.088	0.0802223	0.0802321

300	80.04	-3.66676	20.0008	-0.0049153	1.34491	293.15	293.15	0	353.271	353.271	0.0802606	0.0802715

301	80.2	-3.71456	20.0008	-0.00497912	1.34757	293.15	293.15	0	353.434	353.434	0.0802992	0.0803099

302	80.36	-3.68274	20.0008	-0.00493623	1.35335	293.15	293.15	0	353.6	353.6	0.0803374	0.0803474

303	80.53	-3.57869	20.0008	-0.00479652	1.36055	293.15	293.15	0	353.763	353.763	0.0803757	0.080387

304	80.7	-3.50459	20.0008	-0.00469697	1.3629	293.15	293.15	0	353.929	353.929	0.0804156	0.0804264

305	80.87	-3.46624	19.9956	-0.00464534	1.36847	293.15	293.15	0	354.092	354.092	0.0804537	0.0804648

306	81.04	-3.46271	20.0008	-0.00464037	1.37478	293.15	293.15	0	354.267	354.267	0.0804922	0.0805038

307	81.2	-3.47668	20.0008	-0.00465886	1.38028	293.15	293.15	0	354.42	354.42	0.0805302	0.0805417

308	81.37	-3.51484	20.006	-0.00470976	1.38284	293.15	293.15	0	354.589	354.589	0.0805696	0.0805814

309	81.54	-3.61205	20.0008	-0.00483977	1.38808	293.15	293.15	0	354.762	354.762	0.0806078	0.0806204

310	81.71	-3.69797	20.0008	-0.00495464	1.39148	293.15	293.15	0	354.92	354.92	0.0806466	0.080659

311	81.87	-3.67735	20.0008	-0.00492677	1.39637	293.15	293.15	0	355.092	355.092	0.0806855	0.0806975

312	82.04	-3.62135	20.0008	-0.00485151	1.40317	293.15	293.15	0	355.258	355.258	0.0807241	0.0807359

313	82.21	-3.56789	19.9956	-0.00477964	1.40606	293.15	293.15	0	355.438	355.438	0.0807635	0.0807753

314	82.37	-3.58677	20.0008	-0.00480469	1.41064	293.15	293.15	0	355.595	355.595	0.0808014	0.0808136

315	82.54	-3.62478	20.0008	-0.00485536	1.41475	293.15	293.15	0	355.759	355.759	0.0808393	0.0808522

316	82.7	-3.57696	20.0008	-0.00479108	1.42303	293.15	293.15	0	355.932	355.932	0.0808774	0.08089

317	82.87	-3.4861	20.0008	-0.00466914	1.42669	293.15	293.15	0	356.096	356.096	0.0809163	0.0809292

318	83.04	-3.4208	20.0008	-0.00458145	1.43225	293.15	293.15	0	356.269	356.269	0.0809547	0.0809686

319	83.21	-3.42453	20.0008	-0.00458621	1.43344	293.15	293.15	0	356.426	356.426	0.0809943	0.0810088

320	83.38	-3.48962	20.0008	-0.00467314	1.44037	293.15	293.15	0	356.606	356.606	0.081034	0.0810476

321	83.55	-3.55092	20.0008	-0.00475499	1.44445	293.15	293.15	0	356.756	356.756	0.0810724	0.0810862

322	83.72	-3.5915	20.0008	-0.00480909	1.4478	293.15	293.15	0	356.93	356.93	0.0811112	0.0811253

323	83.88	-3.59358	20.0008	-0.00481163	1.45125	293.15	293.15	0	357.099	357.099	0.0811496	0.0811641

324	84.05	-3.48465	20.0008	-0.00466555	1.45353	293.15	293.15	0	357.258	357.258	0.0811885	0.0812023

325	84.21	-3.36828	20.0008	-0.00450952	1.46042	293.15	293.15	0	357.423	357.423	0.0812272	0.0812403

326	84.38	-3.29028	20.0008	-0.00440486	1.4648	293.15	293.15	0	357.591	357.591	0.0812656	0.0812792

327	84.54	-3.23288	20.0008	-0.0043278	1.47158	293.15	293.15	0	357.769	357.769	0.0813035	0.0813173

328	84.72	-3.26482	20.0008	-0.00437034	1.47525	293.15	293.15	0	357.928	357.928	0.0813425	0.0813571

329	84.88	-3.29991	20.0008	-0.00441708	1.47896	293.15	293.15	0	358.09	358.09	0.081381	0.0813957

330	85.05	-3.34861	19.9956	-0.00448205	1.48576	293.15	293.15	0	358.265	358.265	0.0814196	0.0814342

331	85.21	-3.34738	20.0008	-0.00448019	1.48935	293.15	293.15	0	358.437	358.437	0.0814583	0.0814721

332	85.38	-3.28642	20.0008	-0.00439838	1.493	293.15	293.15	0	358.603	358.603	0.0814962	0.0815107

333	85.55	-3.23126	20.0008	-0.00432434	1.49838	293.15	293.15	0	358.758	358.758	0.0815351	0.0815499

334	85.72	-3.22596	20.0112	-0.00431702	1.50496	293.15	293.15	0	358.94	358.94	0.0815731	0.0815886

335	85.88	-3.19796	20.006	-0.00427934	1.50781	293.15	293.15	0	359.087	359.087	0.0816119	0.0816277

336	86.05	-3.29128	20.0112	-0.00440399	1.51288	293.15	293.15	0	359.26	359.26	0.0816502	0.0816667

337	86.22	-3.38583	20.0019	-0.00453027	1.51691	293.15	293.15	0	359.425	359.425	0.0816893	0.0817058

338	86.39	-3.43982	19.9977	-0.00460229	1.52576	293.15	293.15	0	359.587	359.587	0.0817268	0.081744

339	86.55	-3.45746	19.9904	-0.00462566	1.53058	293.15	293.15	0	359.755	359.755	0.0817656	0.0817825

340	86.72	-3.42164	19.9987	-0.0045775	1.53384	293.15	293.15	0	359.925	359.925	0.0818048	0.0818214

341	86.89	-3.36792	20.0039	-0.00450542	1.53963	293.15	293.15	0	360.101	360.101	0.0818431	0.0818596

342	87.06	-3.36083	20.0112	-0.0044957	1.54372	293.15	293.15	0	360.262	360.262	0.0818823	0.0818991

343	87.22	-3.32674	20.0039	-0.00444986	1.54811	293.15	293.15	0	360.431	360.431	0.0819209	0.0819381

344	87.39	-3.27353	20.0008	-0.00437847	1.55178	293.15	293.15	0	360.599	360.599	0.08196	0.0819764

345	87.55	-3.19167	20.0008	-0.00426877	1.55658	293.15	293.15	0	360.768	360.768	0.0819982	0.0820145

346	87.72	-3.16403	20.0008	-0.0042316	1.5633	293.15	293.15	0	360.923	360.923	0.0820364	0.0820533

347	87.89	-3.16555	20.0008	-0.00423342	1.56902	293.15	293.15	0	361.089	361.089	0.082075	0.0820919

348	88.06	-3.22139	20.0019	-0.00430787	1.57238	293.15	293.15	0	361.255	361.255	0.0821131	0.0821306

349	88.23	-3.2144	20.0102	-0.00429831	1.57466	293.15	293.15	0	361.436	361.436	0.0821527	0.0821702

350	88.39	-3.1648	20.0008	-0.00423178	1.57968	293.15	293.15	0	361.593	361.593	0.0821909	0.0822084

351	88.56	-3.09854	20.0008	-0.00414297	1.58573	293.15	293.15	0	361.756	361.756	0.0822294	0.0822465

352	88.73	-3.07107	20.0008	-0.00410603	1.59007	293.15	293.15	0	361.93	361.93	0.0822679	0.0822858

353	88.89	-3.00817	20.0008	-0.00402173	1.59278	293.15	293.15	0	362.102	362.102	0.0823066	0.0823241

354	89.06	-3.01163	20.0008	-0.00402616	1.59889	293.15	293.15	0	362.266	362.266	0.0823444	0.0823621

355	89.23	-3.01043	19.9977	-0.00402436	1.60751	293.15	293.15	0	362.43	362.43	0.0823829	0.0824011

356	89.39	-3.04493	19.9904	-0.00407026	1.61124	293.15	293.15	0	362.589	362.589	0.0824221	0.0824397

357	89.56	-3.09322	19.9987	-0.00413461	1.61587	293.15	293.15	0	362.763	362.763	0.0824599	0.0824788

358	89.73	-3.07287	20.0029	-0.0041072	1.61994	293.15	293.15	0	362.924	362.924	0.0824981	0.0825168

359	89.89	-3.05601	20.0112	-0.00408447	1.62366	293.15	293.15	0	363.093	363.093	0.0825374	0.0825559

360	90.06	-3.03573	20.0019	-0.00405715	1.62889	293.15	293.15	0	363.261	363.261	0.0825768	0.0825951

361	90.23	-2.92346	19.9925	-0.00390692	1.63466	293.15	293.15	0	363.43	363.43	0.0826149	0.0826332

362	90.4	-2.86315	20.0008	-0.00382612	1.64094	293.15	293.15	0	363.597	363.597	0.0826528	0.082672

363	90.56	-2.84523	20.0008	-0.00380198	1.64501	293.15	293.15	0	363.759	363.759	0.0826906	0.08271

364	90.73	-2.86744	20.0008	-0.00383147	1.64977	293.15	293.15	0	363.933	363.933	0.0827295	0.0827494

365	90.9	-2.93887	20.0008	-0.00392672	1.65497	293.15	293.15	0	364.098	364.098	0.0827683	0.0827883

366	91.06	-3.03206	19.9946	-0.00405103	1.65796	293.15	293.15	0	364.272	364.272	0.0828073	0.0828264

367	91.23	-3.06646	19.9904	-0.00409678	1.66183	293.15	293.15	0	364.426	364.426	0.0828454	0.0828654

368	91.4	-3.04135	20.0008	-0.00406304	1.67043	293.15	293.15	0	364.59	364.59	0.0828841	0.0829042

369	91.57	-3.0581	20.0008	-0.0040852	1.6765	293.15	293.15	0	364.765	364.765	0.0829223	0.082943

370	91.74	-3.08617	20.0008	-0.00412249	1.67763	293.15	293.15	0	364.928	364.928	0.0829608	0.0829816

371	91.9	-3.04126	20.0008	-0.0040623	1.6826	293.15	293.15	0	365.094	365.094	0.0829995	0.08302

372	92.07	-2.98471	19.9914	-0.00398657	1.68796	293.15	293.15	0	365.265	365.265	0.0830379	0.0830583

373	92.24	-2.88688	19.9998	-0.00385571	1.69419	293.15	293.15	0	365.432	365.432	0.0830766	0.0830973

374	92.4	-2.80191	20.0008	-0.00374203	1.70041	293.15	293.15	0	365.602	365.602	0.0831146	0.0831359

375	92.57	-2.71511	20.0008	-0.00362593	1.70382	293.15	293.15	0	365.762	365.762	0.0831529	0.0831735

376	92.74	-2.68477	20.0008	-0.00358524	1.70969	293.15	293.15	0	365.934	365.934	0.0831915	0.0832127

377	92.9	-2.70136	20.0008	-0.00360721	1.71512	293.15	293.15	0	366.086	366.086	0.08323	0.0832515

378	93.07	-2.74382	20.0008	-0.00366372	1.71749	293.15	293.15	0	366.255	366.255	0.0832691	0.0832905

379	93.24	-2.7821	20.0008	-0.00371465	1.7228	293.15	293.15	0	366.428	366.428	0.0833075	0.0833293

380	93.41	-2.73945	20.0008	-0.00365752	1.72712	293.15	293.15	0	366.596	366.596	0.0833461	0.0833679

381	93.57	-2.67794	20.0008	-0.00357521	1.7319	293.15	293.15	0	366.758	366.758	0.083384	0.083406

382	93.74	-2.6532	20.0008	-0.003542	1.7396	293.15	293.15	0	366.924	366.924	0.0834231	0.0834445

383	93.9	-2.65134	20.0008	-0.00353935	1.74381	293.15	293.15	0	367.095	367.095	0.0834611	0.0834823

384	94.07	-2.57977	20.0008	-0.00344364	1.74925	293.15	293.15	0	367.269	367.269	0.0834994	0.0835209

385	94.23	-2.4758	20.0008	-0.00330469	1.75309	293.15	293.15	0	367.416	367.416	0.0835366	0.0835587

386	94.41	-2.45233	19.9956	-0.00327319	1.75988	293.15	293.15	0	367.599	367.599	0.0835762	0.0835984

387	94.57	-2.49715	19.9904	-0.00333285	1.76159	293.15	293.15	0	367.764	367.764	0.0836148	0.0836368

388	94.74	-2.55993	20.0008	-0.00341647	1.76809	293.15	293.15	0	367.936	367.936	0.0836531	0.0836755

389	94.91	-2.64104	20.0008	-0.00352454	1.77465	293.15	293.15	0	368.1	368.1	0.0836917	0.0837139

390	95.07	-2.7036	20.0008	-0.00360784	1.77896	293.15	293.15	0	368.264	368.264	0.08373	0.0837526

391	95.24	-2.74959	20.0008	-0.00366903	1.78486	293.15	293.15	0	368.43	368.43	0.0837685	0.0837914

392	95.41	-2.7928	20.0008	-0.00372651	1.78945	293.15	293.15	0	368.593	368.593	0.0838067	0.0838296

393	95.57	-2.73403	20.0008	-0.00364791	1.79372	293.15	293.15	0	368.76	368.76	0.0838448	0.0838678

394	95.74	-2.66078	20.0008	-0.00355	1.79817	293.15	293.15	0	368.93	368.93	0.0838834	0.0839062

395	95.91	-2.61345	20.0008	-0.00348667	1.80686	293.15	293.15	0	369.097	369.097	0.0839217	0.0839454

396	96.08	-2.61711	20.0008	-0.00349138	1.81043	293.15	293.15	0	369.266	369.266	0.0839603	0.083984

397	96.25	-2.6471	19.9987	-0.00353121	1.8148	293.15	293.15	0	369.427	369.427	0.0839991	0.0840228

398	96.41	-2.65276	19.9904	-0.00353858	1.8211	293.15	293.15	0	369.6	369.6	0.0840375	0.0840612

399	96.58	-2.64753	19.9925	-0.00353143	1.82683	293.15	293.15	0	369.764	369.764	0.0840754	0.0840994

400	96.75	-2.6599	20.0008	-0.00354775	1.83078	293.15	293.15	0	369.922	369.922	0.0841141	0.0841389

401	96.92	-2.66903	20.0008	-0.00355975	1.83473	293.15	293.15	0	370.095	370.095	0.0841534	0.0841777

402	97.08	-2.68168	20.0008	-0.00357645	1.83928	293.15	293.15	0	370.26	370.26	0.0841915	0.0842161

403	97.25	-2.61941	20.0008	-0.00349323	1.84737	293.15	293.15	0	370.424	370.424	0.0842293	0.0842538

404	97.41	-2.54093	20.0008	-0.00338839	1.85284	293.15	293.15	0	370.588	370.588	0.0842674	0.0842925

405	97.58	-2.53803	20.0008	-0.00338435	1.85614	293.15	293.15	0	370.77	370.77	0.0843063	0.0843313

406	97.75	-2.55971	20.0008	-0.00341309	1.85862	293.15	293.15	0	370.925	370.925	0.0843449	0.0843704

407	97.92	-2.56102	19.9914	-0.00341468	1.86423	293.15	293.15	0	371.092	371.092	0.0843833	0.0844084

408	98.09	-2.53604	20.005	-0.0033812	1.8712	293.15	293.15	0	371.263	371.263	0.0844218	0.0844474

409	98.25	-2.52565	20.0008	-0.00336717	1.87713	293.15	293.15	0	371.421	371.421	0.0844605	0.084486

410	98.42	-2.55583	20.0008	-0.00340724	1.88008	293.15	293.15	0	371.592	371.592	0.084499	0.0845241

411	98.58	-2.51852	20.0008	-0.00335733	1.88464	293.15	293.15	0	371.768	371.768	0.0845371	0.0845621

412	98.75	-2.47505	20.0008	-0.00329922	1.89103	293.15	293.15	0	371.929	371.929	0.0845752	0.084601

413	98.92	-2.44248	20.0008	-0.00325565	1.89717	293.15	293.15	0	372.089	372.089	0.0846133	0.0846391

414	99.08	-2.33757	20.0008	-0.00311565	1.90342	293.15	293.15	0	372.266	372.266	0.0846519	0.084677

415	99.25	-2.29068	20.0008	-0.00305299	1.90882	293.15	293.15	0	372.435	372.435	0.0846899	0.0847156

416	99.42	-2.29387	20.0008	-0.0030571	1.91264	293.15	293.15	0	372.6	372.6	0.0847281	0.0847545

417	99.59	-2.36359	19.9998	-0.00314985	1.9212	293.15	293.15	0	372.756	372.756	0.0847662	0.0847926

418	99.76	-2.41667	19.9904	-0.00322043	1.92463	293.15	293.15	0	372.922	372.922	0.0848054	0.0848319

419	99.92	-2.37495	19.9956	-0.00316468	1.9268	293.15	293.15	0	373.096	373.096	0.0848429	0.0848702

420	100.09	-2.32035	19.9904	-0.00309177	1.85862	293.15	293.15	0	373.078	373.078	0.0848812	0.0849085

421	100.22	-2.33183	19.9904	-0.00310694	1.72811	293.15	293.15	0	372.905	372.905	0.0849122	0.0849395

422	100.27	-2.1108	20.0008	-0.00281239	1.61993	293.15	293.15	0	372.74	372.74	0.0849269	0.0849515

423	100.25	-1.14668	20.0008	-0.00152783	1.53561	293.15	293.15	0	372.583	372.583	0.0849246	0.084946

424	100.17	0.538653	20.0008	0.000717716	1.4609	293.15	293.15	0	372.412	372.412	0.0849093	0.0849264

425	100.04	2.78599	20.0008	0.00371227	1.39627	293.15	293.15	0	372.237	372.237	0.0848839	0.0848967

426	99.87	5.29572	20.0008	0.00705678	1.35086	293.15	293.15	0	372.075	372.075	0.0848508	0.0848589

427	99.68	7.95423	20.0008	0.0106	1.31763	293.15	293.15	0	371.916	371.916	0.0848094	0.0848146

428	99.48	10.5079	20.0008	0.0140039	1.29133	293.15	293.15	0	371.737	371.737	0.084765	0.0847674

429	99.25	12.8565	20.0008	0.0171351	1.26762	293.15	293.15	0	371.569	371.569	0.0847161	0.0847154

430	99.02	14.8456	20.0008	0.0197875	1.25391	293.15	293.15	0	371.4	371.4	0.0846662	0.0846628

431	98.79	16.5559	20.0008	0.0220686	1.24639	293.15	293.15	0	371.24	371.24	0.0846144	0.084609

432	98.56	17.9294	20.0008	0.0239011	1.241	293.15	293.15	0	371.067	371.067	0.0845612	0.0845564

433	98.33	18.97	20.0008	0.02529	1.2395	293.15	293.15	0	370.918	370.918	0.0845099	0.0845034

434	98.1	19.7274	20.0008	0.0263016	1.23744	293.15	293.15	0	370.746	370.746	0.0844586	0.084451

435	97.88	20.3171	20.0008	0.0270896	1.23459	293.15	293.15	0	370.573	370.573	0.0844077	0.0843999

436	97.66	20.7776	20.0008	0.0277054	1.23775	293.15	293.15	0	370.415	370.415	0.0843561	0.0843483

437	97.44	21.1032	20.0008	0.0281413	1.24093	293.15	293.15	0	370.252	370.252	0.0843073	0.0842993

438	97.23	21.2632	20.0008	0.0283565	1.23833	293.15	293.15	0	370.079	370.079	0.0842592	0.0842509

439	97.03	21.2482	20.0008	0.0283383	1.24331	293.15	293.15	0	369.906	369.906	0.0842114	0.0842033

440	96.83	21.1333	20.0008	0.0281867	1.24539	293.15	293.15	0	369.732	369.732	0.0841656	0.0841575

441	96.64	20.9764	20.0008	0.027979	1.24783	293.15	293.15	0	369.585	369.585	0.0841205	0.0841131

442	96.45	20.7711	20.0008	0.0277068	1.24585	293.15	293.15	0	369.405	369.405	0.0840767	0.0840692

443	96.26	20.5573	20.0008	0.0274231	1.24521	293.15	293.15	0	369.238	369.238	0.0840326	0.0840264

444	96.08	20.3446	20.0039	0.0271408	1.24213	293.15	293.15	0	369.073	369.073	0.083991	0.0839843

445	95.9	20.0878	20.0112	0.0267998	1.24083	293.15	293.15	0	368.911	368.911	0.0839502	0.0839431

446	95.72	19.836	20.0029	0.0264653	1.24208	293.15	293.15	0	368.744	368.744	0.0839082	0.0839013

447	95.54	19.6475	20.0008	0.0262151	1.23905	293.15	293.15	0	368.57	368.57	0.0838672	0.0838604

448	95.37	19.4845	20.0008	0.0259989	1.23743	293.15	293.15	0	368.402	368.402	0.0838268	0.083821

449	95.2	19.3202	19.9987	0.025781	1.23394	293.15	293.15	0	368.241	368.241	0.0837871	0.0837809

450	95.03	19.1671	19.9925	0.025578	1.23009	293.15	293.15	0	368.073	368.073	0.0837481	0.0837419

451	94.86	19.0171	20.0008	0.0253793	1.22448	293.15	293.15	0	367.904	367.904	0.0837092	0.0837025

452	94.69	18.9032	19.9946	0.0252284	1.21949	293.15	293.15	0	367.738	367.738	0.0836703	0.0836642

453	94.52	18.7823	20.0008	0.0250684	1.2178	293.15	293.15	0	367.583	367.583	0.0836316	0.0836246

454	94.35	18.637	20.0008	0.0248757	1.21594	293.15	293.15	0	367.417	367.417	0.0835917	0.0835859

455	94.19	18.5363	20.0008	0.0247425	1.21006	293.15	293.15	0	367.237	367.237	0.0835545	0.0835479

456	94.02	18.4839	20.0008	0.0246739	1.20407	293.15	293.15	0	367.071	367.071	0.0835152	0.0835084

457	93.85	18.4238	20.0008	0.0245948	1.20148	293.15	293.15	0	366.916	366.916	0.083477	0.0834705

458	93.68	18.3346	20.0008	0.024477	1.19919	293.15	293.15	0	366.743	366.743	0.0834378	0.0834311

459	93.52	18.3063	20.0008	0.0244404	1.19239	293.15	293.15	0	366.569	366.569	0.0834002	0.0833932

460	93.35	18.305	20.0008	0.0244399	1.18727	293.15	293.15	0	366.405	366.405	0.0833622	0.0833545

461	93.18	18.25	20.0008	0.0243677	1.18329	293.15	293.15	0	366.249	366.249	0.0833238	0.083316

462	93.02	18.2051	20.0008	0.0243089	1.17675	293.15	293.15	0	366.068	366.068	0.083285	0.0832774

463	92.85	18.201	20.0008	0.0243047	1.17489	293.15	293.15	0	365.909	365.909	0.0832462	0.0832384

464	92.68	18.2077	20.0008	0.0243149	1.17017	293.15	293.15	0	365.739	365.739	0.0832079	0.0832

465	92.52	18.2086	20.0008	0.0243173	1.16158	293.15	293.15	0	365.572	365.572	0.0831703	0.083162

466	92.35	18.1405	19.9977	0.0242276	1.15871	293.15	293.15	0	365.399	365.399	0.0831318	0.0831238

467	92.19	18.0756	19.9925	0.024142	1.15508	293.15	293.15	0	365.248	365.248	0.0830928	0.0830854

468	92.02	18.0727	20.0008	0.0241394	1.14868	293.15	293.15	0	365.078	365.078	0.0830549	0.083047

469	91.85	18.0845	19.9956	0.0241564	1.14284	293.15	293.15	0	364.905	364.905	0.0830162	0.0830083

470	91.68	18.0563	20.0008	0.0241199	1.13922	293.15	293.15	0	364.738	364.738	0.0829775	0.0829696

471	91.52	17.9884	20.0008	0.0240304	1.1349	293.15	293.15	0	364.568	364.568	0.0829389	0.0829306

472	91.35	17.9274	20.0008	0.0239501	1.13249	293.15	293.15	0	364.401	364.401	0.0828999	0.0828914

473	91.18	17.9076	20.0008	0.0239249	1.12387	293.15	293.15	0	364.238	364.238	0.0828617	0.0828529

474	91.01	17.8883	20.0008	0.0239003	1.12076	293.15	293.15	0	364.065	364.065	0.082823	0.0828145

475	90.85	17.9019	20.0008	0.0239197	1.11659	293.15	293.15	0	363.917	363.917	0.082785	0.0827758

476	90.68	17.9991	20.0008	0.0240507	1.11449	293.15	293.15	0	363.735	363.735	0.0827463	0.0827365

477	90.51	18.0548	19.9966	0.0241265	1.10733	293.15	293.15	0	363.578	363.578	0.082708	0.0826982

478	90.34	18.1123	19.9904	0.0242045	1.09856	293.15	293.15	0	363.406	363.406	0.0826695	0.0826591

479	90.18	18.1338	19.9998	0.0242344	1.09814	293.15	293.15	0	363.241	363.241	0.0826305	0.082621

480	90.01	18.0861	20.0008	0.0241719	1.09232	293.15	293.15	0	363.067	363.067	0.0825923	0.0825818

481	89.84	18.001	20.0008	0.0240594	1.08974	293.15	293.15	0	362.896	362.896	0.0825534	0.0825433

482	89.67	17.8432	20.0008	0.0238497	1.08351	293.15	293.15	0	362.747	362.747	0.0825152	0.0825046

483	89.51	17.7705	19.9925	0.0237537	1.0784	293.15	293.15	0	362.574	362.574	0.0824774	0.082466

484	89.34	17.8034	19.9904	0.0237988	1.07636	293.15	293.15	0	362.404	362.404	0.0824375	0.0824266

485	89.17	17.8811	19.9977	0.0239039	1.07252	293.15	293.15	0	362.244	362.244	0.0823983	0.082388

486	89.01	17.878	19.9956	0.023901	1.06527	293.15	293.15	0	362.075	362.075	0.0823603	0.0823502

487	88.83	17.9246	20.0008	0.0239645	1.06057	293.15	293.15	0	361.906	361.906	0.0823216	0.0823107

488	88.67	17.9538	20.0008	0.0240048	1.05483	293.15	293.15	0	361.74	361.74	0.0822835	0.082272

489	88.5	17.9427	20.0008	0.0239911	1.05327	293.15	293.15	0	361.584	361.584	0.0822446	0.0822333

490	88.33	17.9122	20.0008	0.0239515	1.04778	293.15	293.15	0	361.413	361.413	0.0822063	0.0821951

491	88.17	17.8569	20.0008	0.0238787	1.04211	293.15	293.15	0	361.24	361.24	0.0821674	0.082156

492	88	17.7344	20.0008	0.0237161	1.03748	293.15	293.15	0	361.074	361.074	0.0821291	0.0821181

493	87.84	17.6751	20.0008	0.023638	1.03355	293.15	293.15	0	360.909	360.909	0.0820917	0.0820797

494	87.67	17.6668	20.0008	0.0236281	1.02712	293.15	293.15	0	360.745	360.745	0.082052	0.0820402

495	87.5	17.7183	20.0008	0.0236982	1.02677	293.15	293.15	0	360.57	360.57	0.0820132	0.0820013

496	87.33	17.7688	20.0008	0.023767	1.02379	293.15	293.15	0	360.408	360.408	0.0819737	0.0819617

497	87.16	17.724	19.9966	0.0237082	1.01653	293.15	293.15	0	360.242	360.242	0.0819362	0.0819235

498	86.99	17.6519	19.9904	0.0236129	1.01225	293.15	293.15	0	360.071	360.071	0.0818972	0.0818847

499	86.83	17.6281	19.9998	0.0235822	1.00674	293.15	293.15	0	359.905	359.905	0.0818582	0.081846

500	86.66	17.6287	20.0008	0.0235842	1.00238	293.15	293.15	0	359.734	359.734	0.0818199	0.0818072

501	86.49	17.5971	20.0008	0.0235432	1.00036	293.15	293.15	0	359.575	359.575	0.0817808	0.0817682

502	86.33	17.5731	20.0008	0.0235123	0.996091	293.15	293.15	0	359.401	359.401	0.0817425	0.0817298

503	86.16	17.5399	20.0008	0.023469	0.991582	293.15	293.15	0	359.25	359.25	0.0817037	0.0816914

504	85.99	17.5039	20.0008	0.0234219	0.985235	293.15	293.15	0	359.08	359.08	0.0816656	0.0816529

505	85.82	17.5306	19.9956	0.0234589	0.979897	293.15	293.15	0	358.905	358.905	0.0816272	0.0816138

506	85.66	17.5894	20.0008	0.0235388	0.975752	293.15	293.15	0	358.735	358.735	0.0815885	0.0815754

507	85.49	17.6097	20.0008	0.0235672	0.97287	293.15	293.15	0	358.578	358.578	0.08155	0.0815365

508	85.32	17.6235	20.0008	0.0235868	0.965894	293.15	293.15	0	358.412	358.412	0.0815107	0.0814977

509	85.16	17.5742	19.9998	0.023522	0.963359	293.15	293.15	0	358.241	358.241	0.0814717	0.0814589

510	84.99	17.4691	19.9904	0.0233825	0.95877	293.15	293.15	0	358.065	358.065	0.0814336	0.0814205

511	84.83	17.403	19.9956	0.0232952	0.954194	293.15	293.15	0	357.911	357.911	0.081396	0.0813823

512	84.66	17.4121	20.0008	0.0233086	0.94866	293.15	293.15	0	357.738	357.738	0.081357	0.0813431

513	84.49	17.5301	19.9956	0.0234677	0.942503	293.15	293.15	0	357.573	357.573	0.0813183	0.0813047

514	84.32	17.5953	19.9904	0.0235561	0.941416	293.15	293.15	0	357.399	357.399	0.0812796	0.0812654

515	84.15	17.6026	19.9998	0.0235671	0.936786	293.15	293.15	0	357.253	357.253	0.0812404	0.0812263

516	83.98	17.5826	20.005	0.0235415	0.932626	293.15	293.15	0	357.082	357.082	0.0812018	0.0811876

517	83.81	17.5443	20.0112	0.0234914	0.926889	293.15	293.15	0	356.906	356.906	0.0811634	0.0811481

518	83.65	17.5513	20.0019	0.0235019	0.922701	293.15	293.15	0	356.744	356.744	0.0811244	0.0811099

519	83.49	17.5555	20.0008	0.0235087	0.919421	293.15	293.15	0	356.576	356.576	0.0810864	0.0810718

520	83.31	17.5525	20.0008	0.023506	0.911985	293.15	293.15	0	356.407	356.407	0.0810469	0.0810321

521	83.15	17.526	20.0008	0.0234716	0.908428	293.15	293.15	0	356.238	356.238	0.0810085	0.0809935

522	82.98	17.4553	20.0091	0.0233781	0.904344	293.15	293.15	0	356.07	356.07	0.0809702	0.0809553

523	82.81	17.428	20.0091	0.0233427	0.901357	293.15	293.15	0	355.909	355.909	0.0809311	0.0809159

524	82.65	17.4284	20.0008	0.0233444	0.896316	293.15	293.15	0	355.736	355.736	0.0808922	0.0808771

525	82.48	17.3942	20.0008	0.0232999	0.892262	293.15	293.15	0	355.572	355.572	0.0808534	0.0808382

526	82.31	17.3337	20.0008	0.02322	0.88812	293.15	293.15	0	355.413	355.413	0.0808148	0.0807991

527	82.14	17.2689	20.0008	0.0231343	0.884276	293.15	293.15	0	355.242	355.242	0.0807758	0.0807597

528	81.97	17.2563	20.0008	0.0231187	0.880986	293.15	293.15	0	355.076	355.076	0.0807372	0.0807212

529	81.81	17.2518	20.0008	0.0231137	0.87334	293.15	293.15	0	354.912	354.912	0.0806991	0.0806824

530	81.64	17.226	20.0008	0.0230803	0.870776	293.15	293.15	0	354.747	354.747	0.0806602	0.0806439

531	81.47	17.2569	20.0008	0.0231228	0.867759	293.15	293.15	0	354.575	354.575	0.0806217	0.0806052

532	81.31	17.2949	20.0008	0.023175	0.86591	293.15	293.15	0	354.402	354.402	0.0805824	0.0805661

533	81.14	17.2764	20.0008	0.0231514	0.859946	293.15	293.15	0	354.245	354.245	0.0805441	0.0805274

534	80.97	17.1598	20.0008	0.0229962	0.853659	293.15	293.15	0	354.073	354.073	0.0805052	0.0804888

535	80.81	17.1086	20.0008	0.0229289	0.84944	293.15	293.15	0	353.908	353.908	0.0804669	0.0804502

536	80.64	17.1447	20.005	0.0229784	0.844095	293.15	293.15	0	353.734	353.734	0.0804283	0.080411

537	80.47	17.1904	20.0112	0.0230408	0.840306	293.15	293.15	0	353.582	353.582	0.0803894	0.080372

538	80.3	17.2009	20.0029	0.0230559	0.834621	293.15	293.15	0	353.413	353.413	0.0803508	0.0803329

539	80.13	17.2346	19.9977	0.0231024	0.832278	293.15	293.15	0	353.239	353.239	0.0803115	0.0802937

540	79.97	17.2577	19.9904	0.0231344	0.829647	293.15	293.15	0	353.08	353.08	0.0802734	0.0802553

541	79.8	17.2024	19.9925	0.0230615	0.826064	293.15	293.15	0	352.91	352.91	0.0802337	0.0802164

542	79.63	17.1448	20.0029	0.0229854	0.818561	293.15	293.15	0	352.742	352.742	0.0801958	0.0801769

543	79.46	17.1348	20.0112	0.0229732	0.814301	293.15	293.15	0	352.58	352.58	0.0801566	0.0801384

544	79.3	17.1091	20.005	0.0229398	0.809837	293.15	293.15	0	352.415	352.415	0.0801187	0.0801001

545	79.13	17.0211	20.0008	0.0228231	0.807628	293.15	293.15	0	352.234	352.234	0.0800794	0.080061

546	78.96	16.9951	20.0008	0.0227894	0.804119	293.15	293.15	0	352.077	352.077	0.0800408	0.080022

547	78.79	17.0294	20.0008	0.0228364	0.797226	293.15	293.15	0	351.913	351.913	0.0800022	0.0799829

548	78.63	16.9907	20.0112	0.0227857	0.795116	293.15	293.15	0	351.739	351.739	0.0799633	0.0799445

549	78.46	16.9413	20.0019	0.0227207	0.790157	293.15	293.15	0	351.583	351.583	0.0799247	0.0799058

550	78.29	16.9018	20.0008	0.0226688	0.78857	293.15	293.15	0	351.412	351.412	0.079885	0.0798663

551	78.13	16.9076	20.0008	0.0226777	0.781229	293.15	293.15	0	351.237	351.237	0.0798468	0.0798277

552	77.95	16.9184	20.0008	0.0226934	0.778381	293.15	293.15	0	351.075	351.075	0.0798076	0.079788

553	77.79	16.9055	20.0008	0.0226772	0.774717	293.15	293.15	0	350.916	350.916	0.0797689	0.0797489

554	77.63	16.887	20.0008	0.0226535	0.770236	293.15	293.15	0	350.743	350.743	0.0797313	0.0797114

555	77.46	16.8204	20.0008	0.0225654	0.767018	293.15	293.15	0	350.573	350.573	0.0796924	0.0796722

556	77.29	16.7976	20.0008	0.0225358	0.761076	293.15	293.15	0	350.396	350.396	0.0796527	0.0796324

557	77.12	16.8221	20.0008	0.0225698	0.759042	293.15	293.15	0	350.249	350.249	0.0796141	0.0795936

558	76.95	16.8239	20.006	0.0225734	0.754847	293.15	293.15	0	350.082	350.082	0.0795755	0.079555

559	76.79	16.8404	20.0008	0.0225967	0.74828	293.15	293.15	0	349.903	349.903	0.0795367	0.0795163

560	76.62	16.891	20.0008	0.0226657	0.743099	293.15	293.15	0	349.744	349.744	0.0794985	0.0794774

561	76.45	16.8715	20.0008	0.0226407	0.740322	293.15	293.15	0	349.582	349.582	0.0794593	0.0794388

562	76.28	16.8386	20.0008	0.0225977	0.738749	293.15	293.15	0	349.407	349.407	0.0794203	0.0793994

563	76.11	16.723	20.0008	0.0224438	0.736248	293.15	293.15	0	349.236	349.236	0.0793801	0.0793597

564	75.95	16.6552	20.0008	0.0223538	0.727835	293.15	293.15	0	349.071	349.071	0.0793428	0.0793222

565	75.78	16.6383	20.0008	0.0223323	0.723476	293.15	293.15	0	348.914	348.914	0.0793046	0.0792832

566	75.61	16.6365	20.0008	0.0223309	0.722838	293.15	293.15	0	348.732	348.732	0.079265	0.0792439

567	75.45	16.651	20.0008	0.0223516	0.71678	293.15	293.15	0	348.568	348.568	0.0792267	0.0792052

568	75.28	16.7247	20.0008	0.0224516	0.714474	293.15	293.15	0	348.402	348.402	0.0791883	0.0791669

569	75.11	16.7913	19.9966	0.0225422	0.708179	293.15	293.15	0	348.247	348.247	0.0791489	0.0791274

570	74.95	16.8145	19.9904	0.0225744	0.705036	293.15	293.15	0	348.076	348.076	0.0791103	0.0790884

571	74.78	16.8136	19.9998	0.0225744	0.700349	293.15	293.15	0	347.901	347.901	0.0790717	0.0790499

572	74.61	16.7635	20.0008	0.0225083	0.695443	293.15	293.15	0	347.739	347.739	0.079032	0.0790099

573	74.45	16.6601	20.0008	0.0223706	0.691437	293.15	293.15	0	347.58	347.58	0.0789934	0.078972

574	74.28	16.5937	20.0008	0.0222825	0.687807	293.15	293.15	0	347.406	347.406	0.0789551	0.0789329

575	74.11	16.6015	19.9925	0.0222941	0.683808	293.15	293.15	0	347.243	347.243	0.078917	0.0788943

576	73.94	16.6573	19.9904	0.0223702	0.677596	293.15	293.15	0	347.073	347.073	0.0788773	0.0788542

577	73.77	16.7048	19.9977	0.022435	0.676823	293.15	293.15	0	346.913	346.913	0.0788379	0.0788158

578	73.61	16.7309	19.9956	0.0224712	0.672275	293.15	293.15	0	346.745	346.745	0.0787998	0.0787765

579	73.44	16.7504	20.0008	0.0224986	0.668131	293.15	293.15	0	346.576	346.576	0.0787612	0.0787378

580	73.27	16.7565	20.0071	0.022508	0.663635	293.15	293.15	0	346.408	346.408	0.0787222	0.0786986

581	73.1	16.7388	19.9998	0.0224853	0.661165	293.15	293.15	0	346.246	346.246	0.0786829	0.0786589

582	72.94	16.6804	19.9914	0.022408	0.655027	293.15	293.15	0	346.073	346.073	0.0786445	0.0786212

583	72.77	16.5785	20.0008	0.0222723	0.651162	293.15	293.15	0	345.907	345.907	0.078606	0.0785818

584	72.6	16.5108	19.9998	0.0221823	0.649735	293.15	293.15	0	345.736	345.736	0.0785663	0.0785424

585	72.44	16.5199	19.9904	0.0221957	0.643346	293.15	293.15	0	345.579	345.579	0.0785276	0.0785039

586	72.27	16.5081	19.9904	0.0221811	0.64022	293.15	293.15	0	345.405	345.405	0.0784886	0.0784643

587	72.1	16.4899	20.0008	0.0221576	0.637157	293.15	293.15	0	345.241	345.241	0.07845	0.0784254

588	71.93	16.5086	20.0008	0.022184	0.633149	293.15	293.15	0	345.066	345.066	0.0784113	0.0783871

589	71.77	16.5554	20.0008	0.0222479	0.62893	293.15	293.15	0	344.911	344.911	0.0783725	0.0783481

590	71.6	16.592	20.0008	0.0222983	0.62394	293.15	293.15	0	344.74	344.74	0.0783334	0.078309

591	71.43	16.6185	19.9925	0.0223349	0.6199	293.15	293.15	0	344.581	344.581	0.0782943	0.0782702

592	71.26	16.6235	19.9987	0.0223428	0.618493	293.15	293.15	0	344.412	344.412	0.0782549	0.0782311

593	71.1	16.6216	20.0008	0.0223414	0.611997	293.15	293.15	0	344.244	344.244	0.0782169	0.0781923

594	70.93	16.5894	19.9956	0.0222993	0.607225	293.15	293.15	0	344.065	344.065	0.0781781	0.0781528

595	70.76	16.5237	20.0008	0.0222121	0.605018	293.15	293.15	0	343.915	343.915	0.0781389	0.0781136

596	70.59	16.5222	20.0008	0.0222112	0.600035	293.15	293.15	0	343.737	343.737	0.0781008	0.0780749

597	70.43	16.5622	20.0008	0.022266	0.595652	293.15	293.15	0	343.568	343.568	0.0780619	0.0780361

598	70.26	16.5774	20.0008	0.0222876	0.593511	293.15	293.15	0	343.409	343.409	0.0780229	0.0779966

599	70.09	16.6231	20.0008	0.0223502	0.589733	293.15	293.15	0	343.245	343.245	0.0779834	0.0779581

600	69.92	16.6229	20.0112	0.0223511	0.584771	293.15	293.15	0	343.081	343.081	0.0779451	0.0779183

601	69.76	16.5363	20.0008	0.0222358	0.578909	293.15	293.15	0	342.899	342.899	0.0779058	0.0778798

602	69.59	16.4489	19.9904	0.0221194	0.577033	293.15	293.15	0	342.733	342.733	0.077867	0.07784

603	69.42	16.4584	19.9998	0.0221332	0.575311	293.15	293.15	0	342.578	342.578	0.0778281	0.0778012

604	69.25	16.4595	20.0008	0.0221359	0.572662	293.15	293.15	0	342.399	342.399	0.0777892	0.0777627

605	69.09	16.4469	20.0008	0.02212	0.565737	293.15	293.15	0	342.239	342.239	0.0777497	0.0777236

606	68.92	16.3795	19.9977	0.0220305	0.562373	293.15	293.15	0	342.066	342.066	0.0777117	0.0776853

607	68.75	16.2842	19.9904	0.0219034	0.559636	293.15	293.15	0	341.915	341.915	0.0776726	0.0776458

608	68.59	16.2085	19.9977	0.0218027	0.555136	293.15	293.15	0	341.744	341.744	0.0776337	0.0776068

609	68.42	16.2162	20.0008	0.0218142	0.549311	293.15	293.15	0	341.572	341.572	0.077595	0.0775677

610	68.25	16.2579	20.0008	0.0218713	0.547639	293.15	293.15	0	341.404	341.404	0.0775554	0.0775288

611	68.08	16.2963	20.0008	0.0219241	0.543833	293.15	293.15	0	341.251	341.251	0.0775163	0.0774884

612	67.91	16.2927	20.0008	0.0219204	0.54192	293.15	293.15	0	341.077	341.077	0.0774771	0.0774499

613	67.75	16.289	20.0008	0.0219165	0.534865	293.15	293.15	0	340.905	340.905	0.0774384	0.0774113

614	67.58	16.3298	20.0071	0.0219725	0.532475	293.15	293.15	0	340.739	340.739	0.0773995	0.0773718

615	67.41	16.3431	20.0008	0.0219915	0.528531	293.15	293.15	0	340.583	340.583	0.0773611	0.0773329

616	67.24	16.3158	19.9904	0.0219559	0.525944	293.15	293.15	0	340.402	340.402	0.0773219	0.0772936

617	67.08	16.3121	20.0008	0.021952	0.521222	293.15	293.15	0	340.237	340.237	0.0772839	0.0772554

618	66.91	16.2228	20.0008	0.021833	0.513427	293.15	293.15	0	340.064	340.064	0.0772447	0.0772168

619	66.75	16.163	20.0008	0.0217535	0.512479	293.15	293.15	0	339.908	339.908	0.0772062	0.0771782

620	66.58	16.1699	20.0008	0.021764	0.507472	293.15	293.15	0	339.734	339.734	0.0771678	0.0771388

621	66.41	16.1855	20.0008	0.0217861	0.503557	293.15	293.15	0	339.581	339.581	0.0771277	0.0770986

622	66.24	16.2276	19.9977	0.0218438	0.500256	293.15	293.15	0	339.404	339.404	0.0770887	0.0770597

623	66.08	16.2276	19.9935	0.0218449	0.496232	293.15	293.15	0	339.24	339.24	0.0770508	0.0770216

624	65.91	16.1989	20.0008	0.0218074	0.494186	293.15	293.15	0	339.079	339.079	0.0770115	0.0769824

625	65.74	16.2522	20.0008	0.0218802	0.489556	293.15	293.15	0	338.91	338.91	0.0769729	0.0769431

626	65.57	16.2801	20.0029	0.0219189	0.485547	293.15	293.15	0	338.742	338.742	0.0769329	0.0769034

627	65.4	16.2968	20.0112	0.0219426	0.482332	293.15	293.15	0	338.573	338.573	0.0768937	0.0768633

628	65.23	16.2641	20.0039	0.0218997	0.478194	293.15	293.15	0	338.406	338.406	0.0768545	0.0768245

629	65.07	16.2303	20.0019	0.0218552	0.476801	293.15	293.15	0	338.243	338.243	0.0768153	0.0767858

630	64.9	16.2053	20.0102	0.0218227	0.473149	293.15	293.15	0	338.07	338.07	0.0767761	0.076746

631	64.73	16.189	20.0008	0.0218019	0.467038	293.15	293.15	0	337.905	337.905	0.0767381	0.0767075

632	64.57	16.2276	20.0008	0.0218549	0.464271	293.15	293.15	0	337.742	337.742	0.0766996	0.0766689

633	64.4	16.2618	19.9956	0.021902	0.459219	293.15	293.15	0	337.576	337.576	0.0766607	0.0766297

634	64.24	16.2341	20.0008	0.0218658	0.457184	293.15	293.15	0	337.412	337.412	0.0766213	0.076591

635	64.07	16.1271	20.0008	0.0217228	0.45153	293.15	293.15	0	337.238	337.238	0.0765824	0.0765517

636	63.9	16.0632	20.0008	0.0216378	0.448954	293.15	293.15	0	337.066	337.066	0.0765435	0.0765126

637	63.73	16.0784	20.0008	0.0216595	0.449459	293.15	293.15	0	336.918	336.918	0.0765035	0.0764725

638	63.56	16.1023	20.0008	0.0216927	0.444443	293.15	293.15	0	336.745	336.745	0.0764649	0.0764341

639	63.4	16.0923	20.0008	0.0216804	0.435211	293.15	293.15	0	336.574	336.574	0.0764269	0.0763952

640	63.23	16.0688	20.0008	0.0216498	0.432894	293.15	293.15	0	336.4	336.4	0.0763878	0.0763561

641	63.06	16.151	20.0008	0.0217617	0.430238	293.15	293.15	0	336.241	336.241	0.0763485	0.0763162

642	62.89	16.1951	20.0008	0.0218221	0.426047	293.15	293.15	0	336.069	336.069	0.0763094	0.0762774

643	62.73	16.1982	20.0008	0.0218274	0.420901	293.15	293.15	0	335.904	335.904	0.0762708	0.0762382

644	62.56	16.2	20.0008	0.021831	0.420251	293.15	293.15	0	335.743	335.743	0.0762311	0.0761987

645	62.39	16.2328	20.0008	0.0218763	0.41678	293.15	293.15	0	335.583	335.583	0.0761928	0.07616

646	62.22	16.2034	20.0008	0.0218378	0.412783	293.15	293.15	0	335.406	335.406	0.0761536	0.0761209

647	62.06	16.15	20.0008	0.0217669	0.407193	293.15	293.15	0	335.238	335.238	0.0761146	0.0760819

648	61.89	16.1231	20.0029	0.0217317	0.403954	293.15	293.15	0	335.064	335.064	0.0760751	0.0760426

649	61.72	16.1731	20.0112	0.0218003	0.402118	293.15	293.15	0	334.915	334.915	0.0760353	0.0760023

650	61.55	16.2147	20.0102	0.0218574	0.398626	293.15	293.15	0	334.734	334.734	0.0759971	0.0759637

651	61.39	16.2287	20.0008	0.0218775	0.395308	293.15	293.15	0	334.587	334.587	0.0759586	0.0759249

652	61.22	16.2533	20.0008	0.0219117	0.389765	293.15	293.15	0	334.404	334.404	0.0759196	0.0758858

653	61.05	16.2988	20.0008	0.0219742	0.386863	293.15	293.15	0	334.239	334.239	0.075881	0.075847

654	60.89	16.3299	20.0008	0.0220172	0.383723	293.15	293.15	0	334.067	334.067	0.0758413	0.0758077

655	60.72	16.3217	20.0008	0.0220072	0.380556	293.15	293.15	0	333.919	333.919	0.0758022	0.0757687

656	60.55	16.2848	20.0008	0.0219586	0.373689	293.15	293.15	0	333.739	333.739	0.0757635	0.0757292

657	60.38	16.1983	20.0008	0.0218431	0.37081	293.15	293.15	0	333.573	333.573	0.0757239	0.0756899

658	60.21	16.1191	20.0008	0.0217374	0.37082	293.15	293.15	0	333.411	333.411	0.0756846	0.0756508

659	60.05	16.0266	20.0008	0.0216138	0.366839	293.15	293.15	0	333.243	333.243	0.0756459	0.0756112

660	59.88	15.9586	20.0008	0.0215231	0.358773	293.15	293.15	0	333.073	333.073	0.0756083	0.0755724

661	59.71	15.9169	20.0008	0.021468	0.3579	293.15	293.15	0	332.912	332.912	0.0755683	0.0755335

662	59.54	15.9646	20.0008	0.0215334	0.355549	293.15	293.15	0	332.745	332.745	0.0755288	0.0754936

663	59.37	16.0748	20.0008	0.0216831	0.351899	293.15	293.15	0	332.576	332.576	0.0754901	0.0754539

664	59.21	16.1151	20.0008	0.0217386	0.347728	293.15	293.15	0	332.408	332.408	0.0754509	0.0754146

665	59.04	16.1277	20.0008	0.0217567	0.344185	293.15	293.15	0	332.236	332.236	0.0754122	0.0753752

666	58.87	16.1174	20.0008	0.0217439	0.340212	293.15	293.15	0	332.08	332.08	0.0753726	0.0753366

667	58.71	16.0779	20.0008	0.0216917	0.337762	293.15	293.15	0	331.916	331.916	0.0753335	0.0752974

668	58.54	16.042	20.0008	0.0216444	0.336091	293.15	293.15	0	331.743	331.743	0.0752938	0.0752576

669	58.37	16.002	20.0008	0.0215915	0.328044	293.15	293.15	0	331.57	331.57	0.0752554	0.0752191

670	58.2	15.9597	19.9904	0.0215355	0.325453	293.15	293.15	0	331.396	331.396	0.0752162	0.0751797

671	58.04	15.9572	19.9998	0.0215333	0.3215	293.15	293.15	0	331.249	331.249	0.0751774	0.0751406

672	57.87	15.9638	19.9956	0.0215432	0.321381	293.15	293.15	0	331.076	331.076	0.0751375	0.0751007

673	57.7	16.0119	20.0008	0.0216093	0.317589	293.15	293.15	0	330.904	330.904	0.0750992	0.0750623

674	57.54	16.0526	20.0008	0.0216653	0.310455	293.15	293.15	0	330.737	330.737	0.0750602	0.0750232

675	57.37	16.0618	20.0039	0.0216789	0.306491	293.15	293.15	0	330.576	330.576	0.0750221	0.0749845

676	57.21	16.8736	20.0081	0.0227756	0.28708	293.15	293.15	0	330.408	330.408	0.0749902	0.0749471

677	57.07	20.3693	20.0008	0.0274951	0.249393	293.15	293.15	0	330.251	330.251	0.0749695	0.074914

678	56.94	25.7607	20.0008	0.034774	0.203515	293.15	293.15	0	330.083	330.083	0.0749504	0.0748842

679	56.8	32.0553	20.0008	0.0432729	0.15814	293.15	293.15	0	329.905	329.905	0.074928	0.0748515

680	56.65	38.1212	20.0008	0.0514638	0.125657	293.15	293.15	0	329.746	329.746	0.0749002	0.0748157

681	56.48	44.1139	20.0008	0.059557	0.0972338	293.15	293.15	0	329.585	329.585	0.0748676	0.0747763

682	56.3	50.0089	20.0008	0.0675194	0.0660874	293.15	293.15	0	329.41	329.41	0.0748346	0.0747348

683	56.12	55.8189	20.0008	0.075368	0.0345959	293.15	293.15	0	329.239	329.239	0.0748004	0.0746922

684	55.94	61.5752	20.0008	0.083145	0.0105955	293.15	293.15	0	329.065	329.065	0.0747632	0.0746483

685	55.74	66.9645	20.0008	0.0904275	-0.00679403	293.15	293.15	0	328.917	328.917	0.0747233	0.0746018

686	55.55	71.7148	19.9956	0.0968479	-0.0227396	293.15	293.15	0	328.744	328.744	0.0746818	0.0745566

687	55.36	75.6408	19.9904	0.102155	-0.0473474	293.15	293.15	0	328.57	328.57	0.0746424	0.0745136

688	55.18	78.8291	20.0008	0.106467	-0.0699477	293.15	293.15	0	328.406	328.406	0.0746037	0.0744714

689	55.02	81.4522	20.0008	0.110015	-0.0960592	293.15	293.15	0	328.234	328.234	0.0745668	0.0744326

690	54.85	83.6131	20.0008	0.11294	-0.120819	293.15	293.15	0	328.07	328.07	0.0745305	0.0743941

691	54.7	85.3135	20.0008	0.115242	-0.152144	293.15	293.15	0	327.904	327.904	0.0744959	0.0743576

692	54.54	86.6367	20.0008	0.117035	-0.184144	293.15	293.15	0	327.732	327.732	0.0744608	0.0743218

693	54.4	87.5257	20.0008	0.118241	-0.211738	293.15	293.15	0	327.583	327.583	0.0744258	0.074287

694	54.25	88.0956	20.0008	0.119016	-0.245825	293.15	293.15	0	327.404	327.404	0.0743914	0.0742524

695	54.1	88.395	20.0008	0.119426	-0.282839	293.15	293.15	0	327.236	327.236	0.0743566	0.0742175

696	53.95	88.4661	20.0008	0.119528	-0.315491	293.15	293.15	0	327.07	327.07	0.0743217	0.0741836

697	53.81	88.3239	20.0008	0.119341	-0.348638	293.15	293.15	0	326.915	326.915	0.074288	0.0741493

698	53.66	88.0674	20.0008	0.118999	-0.3845	293.15	293.15	0	326.748	326.748	0.0742534	0.074115

699	53.52	87.4541	20.0008	0.118176	-0.4221	293.15	293.15	0	326.569	326.569	0.0742165	0.0740804

700	53.36	86.5103	20.0008	0.116906	-0.452281	293.15	293.15	0	326.411	326.411	0.0741782	0.0740445

701	53.21	85.357	20.0019	0.115353	-0.482486	293.15	293.15	0	326.248	326.248	0.0741405	0.0740087

702	53.05	83.9851	20.0102	0.113504	-0.511388	293.15	293.15	0	326.074	326.074	0.074101	0.073972

703	52.89	82.3117	20.0008	0.111248	-0.533758	293.15	293.15	0	325.919	325.919	0.0740592	0.073933

704	52.72	80.2761	20.0008	0.108503	-0.558891	293.15	293.15	0	325.745	325.745	0.0740162	0.0738937

705	52.54	77.9656	20.0008	0.105385	-0.573639	293.15	293.15	0	325.571	325.571	0.0739704	0.0738514

706	52.35	75.3059	20.0039	0.101796	-0.584827	293.15	293.15	0	325.408	325.408	0.0739223	0.0738076

707	52.16	72.2228	20.0112	0.0976342	-0.586034	293.15	293.15	0	325.242	325.242	0.0738711	0.073762

708	51.95	68.6938	20.0019	0.0928694	-0.578028	293.15	293.15	0	325.071	325.071	0.0738159	0.0737126

709	51.73	64.73	20.0008	0.0875166	-0.564391	293.15	293.15	0	324.921	324.921	0.0737568	0.0736602

710	51.49	60.2887	20.0008	0.0815177	-0.536194	293.15	293.15	0	324.743	324.743	0.073695	0.0736045

711	51.24	55.3759	20.0008	0.0748807	-0.492503	293.15	293.15	0	324.575	324.575	0.0736277	0.0735452

712	50.96	50.2095	20.0008	0.0679002	-0.440351	293.15	293.15	0	324.402	324.402	0.0735571	0.0734808

713	50.68	45.282	20.0008	0.0612418	-0.387249	293.15	293.15	0	324.25	324.25	0.0734857	0.0734151

714	50.4	40.8542	20.0008	0.0552582	-0.319697	293.15	293.15	0	324.08	324.08	0.0734144	0.0733478

715	50.11	37.1155	20.0008	0.0502057	-0.24557	293.15	293.15	0	323.908	323.908	0.0733437	0.0732803

716	49.82	33.9905	20.0008	0.0459826	-0.169426	293.15	293.15	0	323.74	323.74	0.0732729	0.0732117

717	49.53	31.5268	20.0008	0.0426535	-0.0917554	293.15	293.15	0	323.57	323.57	0.0732041	0.0731448

718	49.25	29.5922	20.0008	0.0400395	-0.0107617	293.15	293.15	0	323.402	323.402	0.0731367	0.0730788

719	48.97	28.0916	20.0008	0.0380123	0.0702188	293.15	293.15	0	323.248	323.248	0.0730705	0.0730125

720	48.73	26.9964	20.0008	0.0365329	0.144243	293.15	293.15	0	323.075	323.075	0.0730145	0.0729573

721	48.57	25.7433	20.0008	0.034839	0.188879	293.15	293.15	0	322.91	322.91	0.0729731	0.0729185

722	48.45	23.9938	20.006	0.0324725	0.218584	293.15	293.15	0	322.736	322.736	0.0729417	0.0728907

723	48.35	21.9442	20.0112	0.0296995	0.233621	293.15	293.15	0	322.581	322.581	0.0729159	0.0728676

724	48.28	19.8185	19.9925	0.0268232	0.240323	293.15	293.15	0	322.41	322.41	0.0728947	0.0728492

725	48.2	17.8726	20.0039	0.0241901	0.243038	293.15	293.15	0	322.243	322.243	0.0728751	0.0728321

726	48.13	16.1699	20.0112	0.0218861	0.238279	293.15	293.15	0	322.063	322.063	0.0728565	0.072815

727	48.05	14.7006	20.0029	0.0198977	0.230592	293.15	293.15	0	321.904	321.904	0.0728374	0.0727972

728	47.97	13.5157	20.0008	0.0182945	0.220963	293.15	293.15	0	321.735	321.735	0.0728175	0.0727773

729	47.88	12.6524	19.9987	0.0171264	0.212507	293.15	293.15	0	321.583	321.583	0.0727958	0.0727561

730	47.78	12.096	19.9904	0.0163737	0.199629	293.15	293.15	0	321.407	321.407	0.072773	0.0727332

731	47.68	11.8102	19.9914	0.0159873	0.188778	293.15	293.15	0	321.254	321.254	0.072748	0.0727087

732	47.57	11.6999	20.0008	0.0158385	0.176159	293.15	293.15	0	321.078	321.078	0.0727223	0.0726826

733	47.45	11.7279	20.0008	0.0158771	0.165217	293.15	293.15	0	320.907	320.907	0.0726949	0.072654

734	47.32	11.8906	20.0008	0.0160979	0.153837	293.15	293.15	0	320.734	320.734	0.072666	0.0726244

735	47.18	12.0664	20.0008	0.0163366	0.146843	293.15	293.15	0	320.587	320.587	0.0726348	0.0725919

736	47.04	12.3198	20.0008	0.0166804	0.135746	293.15	293.15	0	320.404	320.404	0.0726031	0.0725597

737	46.9	12.6482	20.0008	0.0171258	0.129132	293.15	293.15	0	320.24	320.24	0.0725691	0.0725253

738	46.75	13.0204	20.0008	0.0176306	0.121947	293.15	293.15	0	320.067	320.067	0.0725352	0.0724907

739	46.6	13.3707	20.0008	0.0181057	0.114335	293.15	293.15	0	319.911	319.911	0.0725004	0.0724559

740	46.45	13.7176	20.0008	0.0185764	0.106221	293.15	293.15	0	319.729	319.729	0.0724642	0.0724189

741	46.28	14.0786	20.0008	0.0190661	0.103022	293.15	293.15	0	319.58	319.58	0.072426	0.0723801

742	46.12	14.3216	20.0008	0.0193962	0.0999636	293.15	293.15	0	319.407	319.407	0.0723889	0.0723428

743	45.97	14.4821	20.0008	0.0196144	0.094026	293.15	293.15	0	319.237	319.237	0.0723522	0.0723061

744	45.81	14.614	19.9925	0.0197941	0.0854471	293.15	293.15	0	319.079	319.079	0.0723149	0.072268

745	45.64	14.7821	19.9977	0.0200228	0.0834894	293.15	293.15	0	318.913	318.913	0.072277	0.0722299

746	45.48	14.9737	20.0008	0.0202833	0.0814255	293.15	293.15	0	318.746	318.746	0.0722376	0.0721906

747	45.31	15.0927	20.0008	0.0204455	0.0760257	293.15	293.15	0	318.567	318.567	0.0721986	0.0721512

748	45.14	15.1856	20.0008	0.0205724	0.0747017	293.15	293.15	0	318.408	318.408	0.0721595	0.072112

749	44.98	15.2745	20.0008	0.020694	0.071447	293.15	293.15	0	318.237	318.237	0.0721205	0.0720731

750	44.81	15.3655	20.0008	0.0208182	0.0646434	293.15	293.15	0	318.071	318.071	0.0720829	0.0720341

751	44.64	15.384	20.0008	0.0208444	0.0642665	293.15	293.15	0	317.915	317.915	0.0720426	0.0719943

752	44.47	15.3919	20.0008	0.0208561	0.0602054	293.15	293.15	0	317.742	317.742	0.0720035	0.0719544

753	44.31	15.471	20.006	0.0209644	0.0591754	293.15	293.15	0	317.569	317.569	0.0719639	0.0719156

754	44.14	15.5177	20.0112	0.0210287	0.0560592	293.15	293.15	0	317.405	317.405	0.0719245	0.0718763

755	43.97	15.5662	20.0019	0.0210956	0.0542991	293.15	293.15	0	317.249	317.249	0.071885	0.0718364

756	43.81	15.5643	20.0008	0.021094	0.050481	293.15	293.15	0	317.069	317.069	0.0718459	0.0717974

757	43.64	15.5323	20.0008	0.0210518	0.0458204	293.15	293.15	0	316.902	316.902	0.0718069	0.0717584

758	43.48	15.5309	20.0008	0.0210509	0.0439604	293.15	293.15	0	316.736	316.736	0.0717685	0.0717192

759	43.3	15.5975	20.0008	0.0211422	0.0392664	293.15	293.15	0	316.576	316.576	0.0717284	0.0716781

760	43.13	15.6143	20.0008	0.0211661	0.0390361	293.15	293.15	0	316.408	316.408	0.0716882	0.0716386

761	42.96	15.5935	20.0008	0.021139	0.0371292	293.15	293.15	0	316.235	316.235	0.0716482	0.0715982

762	42.8	15.6017	20.0008	0.0211513	0.0349408	293.15	293.15	0	316.074	316.074	0.0716084	0.071559

763	42.63	15.6031	20.0008	0.0211542	0.0308835	293.15	293.15	0	315.905	315.905	0.0715698	0.0715193

764	42.46	15.5599	19.9956	0.0210967	0.0292995	293.15	293.15	0	315.737	315.737	0.0715304	0.0714804

765	42.29	15.4829	20.0008	0.0209934	0.0268278	293.15	293.15	0	315.568	315.568	0.0714907	0.0714406

766	42.12	15.4544	20.0008	0.0209558	0.0273039	293.15	293.15	0	315.402	315.402	0.0714508	0.0714006

767	41.96	15.4581	20.0008	0.020962	0.0214668	293.15	293.15	0	315.247	315.247	0.0714112	0.0713607

768	41.78	15.436	19.9998	0.020933	0.0212436	293.15	293.15	0	315.081	315.081	0.0713714	0.0713205

769	41.62	15.397	19.9904	0.0208812	0.0197943	293.15	293.15	0	314.9	314.9	0.0713326	0.0712817

770	41.45	15.3536	19.9956	0.0208234	0.01894	293.15	293.15	0	314.735	314.735	0.0712924	0.0712417

771	41.28	15.3443	19.9904	0.0208119	0.0163079	293.15	293.15	0	314.58	314.58	0.0712526	0.071202

772	41.11	15.3501	19.9956	0.0208208	0.0136834	293.15	293.15	0	314.407	314.407	0.0712135	0.0711615

773	40.95	15.4024	19.9904	0.0208928	0.00991337	293.15	293.15	0	314.233	314.233	0.0711751	0.0711232

774	40.78	15.4689	20.0008	0.0209841	0.007625	293.15	293.15	0	314.07	314.07	0.0711367	0.0710842

775	40.62	15.4908	20.0008	0.0210148	-0.000320923	293.15	293.15	0	313.904	313.904	0.071098	0.0710465

776	40.47	15.4333	20.0008	0.0209378	-0.00590422	293.15	293.15	0	313.732	313.732	0.0710606	0.0710092

777	40.31	15.296	20.0008	0.0207525	-0.0117071	293.15	293.15	0	313.582	313.582	0.0710233	0.0709717

778	40.15	15.146	20.0008	0.02055	-0.0201835	293.15	293.15	0	313.404	313.404	0.0709876	0.0709356

779	40	15.0338	20.0008	0.0203987	-0.0337138	293.15	293.15	0	313.236	313.236	0.0709516	0.0708993

780	39.85	14.9357	20.0008	0.0202665	-0.0445231	293.15	293.15	0	313.067	313.067	0.0709158	0.070864

781	39.7	14.8963	20.0008	0.020214	-0.0577449	293.15	293.15	0	312.907	312.907	0.070881	0.0708293

782	39.56	14.8531	20.0008	0.0201563	-0.0737543	293.15	293.15	0	312.733	312.733	0.0708463	0.070795

783	39.41	14.7844	20.0008	0.0200639	-0.0893677	293.15	293.15	0	312.584	312.584	0.0708133	0.0707607

784	39.27	14.6062	19.9998	0.019823	-0.107806	293.15	293.15	0	312.412	312.412	0.0707791	0.0707271

785	39.13	14.3883	19.9914	0.0195281	-0.130653	293.15	293.15	0	312.239	312.239	0.0707458	0.0706942

786	38.99	14.2219	20.0008	0.019303	-0.153108	293.15	293.15	0	312.073	312.073	0.0707132	0.0706614

787	38.86	14.0467	20.0008	0.019066	-0.179243	293.15	293.15	0	311.91	311.91	0.0706815	0.0706304

788	38.73	13.83	20.0008	0.0187726	-0.207365	293.15	293.15	0	311.736	311.736	0.0706504	0.0705986

789	38.6	13.663	20.0008	0.0185466	-0.237383	293.15	293.15	0	311.581	311.581	0.0706191	0.0705679

790	38.46	13.5625	20.0008	0.018411	-0.270758	293.15	293.15	0	311.406	311.406	0.0705885	0.0705366

791	38.34	13.4393	20.0008	0.0182444	-0.304697	293.15	293.15	0	311.235	311.235	0.0705569	0.0705066

792	38.21	13.3307	20.0008	0.0180977	-0.341935	293.15	293.15	0	311.067	311.067	0.0705277	0.0704764

793	38.08	13.2511	20.0008	0.0179903	-0.382094	293.15	293.15	0	310.913	310.913	0.0704981	0.0704466

794	37.96	13.1978	20.0008	0.0179186	-0.424426	293.15	293.15	0	310.743	310.743	0.0704693	0.070418

795	37.84	13.1543	20.0008	0.0178603	-0.471295	293.15	293.15	0	310.566	310.566	0.0704409	0.0703889

796	37.72	13.0561	20.0008	0.0177276	-0.516992	293.15	293.15	0	310.405	310.405	0.0704119	0.0703602

797	37.6	12.893	20.0008	0.0175067	-0.566193	293.15	293.15	0	310.245	310.245	0.0703839	0.0703328

798	37.48	12.724	20.0008	0.0172779	-0.624156	293.15	293.15	0	310.072	310.072	0.0703569	0.0703053

799	37.37	12.6067	20.0008	0.0171192	-0.681891	293.15	293.15	0	309.904	309.904	0.0703301	0.0702793

800	37.26	12.5785	20.0008	0.0170815	-0.739323	293.15	293.15	0	309.744	309.744	0.0703033	0.0702517

801	37.15	12.4998	20.0008	0.0169752	-0.801802	293.15	293.15	0	309.576	309.576	0.0702769	0.0702259

802	37.04	12.372	20.0008	0.0168022	-0.871325	293.15	293.15	0	309.405	309.405	0.0702506	0.0701997

803	36.93	12.2486	20.0008	0.0166352	-0.941793	293.15	293.15	0	309.232	309.232	0.0702247	0.0701737

804	36.82	12.1388	20.0008	0.0164866	-1.01181	293.15	293.15	0	309.074	309.074	0.0702002	0.0701485

805	36.71	11.9913	20.0008	0.0162868	-1.08084	293.15	293.15	0	308.92	308.92	0.0701746	0.0701234

806	36.62	11.8939	20.0008	0.0161549	-1.16975	293.15	293.15	0	308.738	308.738	0.0701498	0.0701

807	36.51	11.8221	20.0008	0.016058	-1.25104	293.15	293.15	0	308.574	308.574	0.0701257	0.0700754

808	36.41	11.7004	20.0008	0.0158932	-1.34199	293.15	293.15	0	308.4	308.4	0.0701024	0.0700511

809	36.31	11.6041	20.0008	0.0157628	-1.42543	293.15	293.15	0	308.243	308.243	0.0700786	0.0700279

810	36.21	11.5264	20.0008	0.0156577	-1.52425	293.15	293.15	0	308.07	308.07	0.0700551	0.0700053

811	36.12	11.4668	20.0008	0.0155772	-1.62518	293.15	293.15	0	307.899	307.899	0.0700322	0.0699819

812	36.02	11.4764	20.0008	0.0155907	-1.71713	293.15	293.15	0	307.749	307.749	0.0700101	0.0699593

813	35.93	11.5089	20.0008	0.0156353	-1.82634	293.15	293.15	0	307.576	307.576	0.0699882	0.0699373

814	35.83	11.451	20.0008	0.0155572	-1.93781	293.15	293.15	0	307.407	307.407	0.0699658	0.0699147

815	35.75	11.3331	20.0008	0.0153973	-2.04725	293.15	293.15	0	307.246	307.246	0.0699446	0.0698946

816	35.66	11.1694	20.0008	0.0151754	-2.1649	293.15	293.15	0	307.079	307.079	0.0699237	0.069873

817	35.57	11.0287	20.0008	0.0149845	-2.29505	293.15	293.15	0	306.9	306.9	0.0699023	0.0698523

818	35.48	10.9217	20.0008	0.0148396	-2.41398	293.15	293.15	0	306.742	306.742	0.0698815	0.0698313

819	35.39	10.8864	20.0008	0.0147921	-2.53894	293.15	293.15	0	306.579	306.579	0.0698605	0.0698098

820	35.3	10.8612	20.0008	0.0147582	-2.68087	293.15	293.15	0	306.404	306.404	0.0698407	0.06979

821	35.22	10.7811	20.0008	0.0146498	-2.82205	293.15	293.15	0	306.232	306.232	0.0698206	0.0697705

822	35.13	10.6536	20.0008	0.0144769	-2.95388	293.15	293.15	0	306.078	306.078	0.0698013	0.0697497

823	35.05	10.5537	20.0008	0.0143415	-3.09854	293.15	293.15	0	305.912	305.912	0.0697808	0.0697298

824	34.97	10.4639	20.0008	0.0142198	-3.2477	293.15	293.15	0	305.748	305.748	0.0697619	0.0697118

825	34.89	10.3811	20.0008	0.0141077	-3.40858	293.15	293.15	0	305.575	305.575	0.0697436	0.0696928

826	34.82	10.3135	20.0008	0.0140161	-3.57603	293.15	293.15	0	305.402	305.402	0.0697257	0.0696748

827	34.74	10.2609	20.0008	0.0139449	-3.73058	293.15	293.15	0	305.245	305.245	0.0697075	0.0696576

828	34.67	10.1708	20.0008	0.0138227	-3.9059	293.15	293.15	0	305.073	305.073	0.0696896	0.0696398

829	34.59	10.1033	20.0008	0.0137314	-4.0785	293.15	293.15	0	304.908	304.908	0.0696718	0.0696222

830	34.52	10.0227	20.0008	0.0136221	-4.26338	293.15	293.15	0	304.734	304.734	0.0696545	0.0696042

831	34.45	9.96048	20.0008	0.0135378	-4.43291	293.15	293.15	0	304.582	304.582	0.0696378	0.0695873

832	34.38	9.88802	20.0008	0.0134396	-4.62178	293.15	293.15	0	304.414	304.414	0.0696209	0.0695704

833	34.3	9.80499	20.0008	0.0133271	-4.82091	293.15	293.15	0	304.24	304.24	0.0696034	0.0695532

834	34.23	9.7612	20.0008	0.0132678	-5.00947	293.15	293.15	0	304.08	304.08	0.0695871	0.0695368

835	34.16	9.71966	20.0008	0.0132117	-5.21522	293.15	293.15	0	303.91	303.91	0.0695706	0.0695204

836	34.09	9.66285	19.9956	0.0131347	-5.42421	293.15	293.15	0	303.742	303.742	0.0695542	0.0695039

837	34.03	9.62747	20.0008	0.0130869	-5.63952	293.15	293.15	0	303.573	303.573	0.0695387	0.0694882

838	33.97	9.55364	20.0008	0.0129868	-5.85838	293.15	293.15	0	303.405	303.405	0.0695231	0.0694734

839	33.9	9.45552	20.0008	0.0128537	-6.07528	293.15	293.15	0	303.244	303.244	0.0695087	0.0694581
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RT54.txt
# Name: RT54 2

# Date: Tue May 21 10:28:02 2024

# Weight: 12.5 mg

Time(s)	Temperature(°C)	Heat flow(mW)	Gas 1(sccm/min)	DSC_RAW(µV)	POWER(%)	TEMP_CJR_FURNACE(K)	TEMP_CJR_SAMPLE(K)	TEMP_FURNACE(K)	TEMP_NOM_FURNACE(K)	TEMP_NOM_SAMPLE(K)	VOLTAGE_REFERENCE(V)	VOLTAGE_SAMPLE(V)

0	29.85	-0.15798	19.9904	-0.000215022	0.0935606	293.15	293.15	0	303.259	303.259	0.0685522	0.0684977

1	29.87	-0.433124	20.0008	-0.000589508	0.158795	293.15	293.15	0	303.433	303.433	0.0685559	0.0685026

2	29.95	-1.0137	19.9966	-0.00137967	0.206623	293.15	293.15	0	303.598	303.598	0.0685716	0.0685214

3	30.07	-2.2415	19.9946	-0.00305063	0.238928	293.15	293.15	0	303.761	303.761	0.0685977	0.06855

4	30.22	-3.92233	20.0008	-0.00533795	0.264292	293.15	293.15	0	303.926	303.926	0.0686302	0.0685856

5	30.39	-5.7318	20.0008	-0.00780008	0.287165	293.15	293.15	0	304.099	304.099	0.0686675	0.0686259

6	30.57	-7.56289	20.0008	-0.0102913	0.296326	293.15	293.15	0	304.262	304.262	0.0687091	0.0686701

7	30.76	-9.25813	20.0008	-0.0125974	0.306651	293.15	293.15	0	304.43	304.43	0.0687528	0.0687149

8	30.95	-10.7775	20.0008	-0.0146639	0.311889	293.15	293.15	0	304.6	304.6	0.0687968	0.0687603

9	31.16	-12.1403	20.0008	-0.0165171	0.317364	293.15	293.15	0	304.767	304.767	0.068842	0.0688083

10	31.35	-13.2178	20.0008	-0.017982	0.321468	293.15	293.15	0	304.933	304.933	0.0688867	0.0688543

11	31.55	-14.0251	19.9987	-0.0190792	0.320666	293.15	293.15	0	305.091	305.091	0.0689324	0.0689005

12	31.74	-14.576	19.9904	-0.0198274	0.318923	293.15	293.15	0	305.261	305.261	0.068978	0.0689462

13	31.93	-14.8864	19.9977	-0.0202485	0.320111	293.15	293.15	0	305.434	305.434	0.0690227	0.0689909

14	32.11	-15.0888	20.0008	-0.0205227	0.321923	293.15	293.15	0	305.602	305.602	0.0690668	0.0690342

15	32.29	-15.1716	19.9946	-0.0206342	0.322023	293.15	293.15	0	305.756	305.756	0.0691096	0.0690777

16	32.48	-15.1062	19.9904	-0.020544	0.322821	293.15	293.15	0	305.928	305.928	0.0691527	0.069121

17	32.65	-15.0214	19.9914	-0.0204276	0.324208	293.15	293.15	0	306.092	306.092	0.069195	0.0691628

18	32.83	-14.9421	20.0008	-0.0203186	0.326427	293.15	293.15	0	306.258	306.258	0.0692368	0.0692045

19	33.01	-14.8708	20.0008	-0.0202207	0.327505	293.15	293.15	0	306.429	306.429	0.0692789	0.069247

20	33.18	-14.8013	19.9998	-0.020125	0.327877	293.15	293.15	0	306.603	306.603	0.0693206	0.0692878

21	33.36	-14.7195	19.9904	-0.0200128	0.333104	293.15	293.15	0	306.769	306.769	0.0693612	0.0693288

22	33.53	-14.5896	19.9966	-0.0198351	0.334285	293.15	293.15	0	306.93	306.93	0.0694017	0.0693698

23	33.7	-14.3829	19.9904	-0.019553	0.337548	293.15	293.15	0	307.087	307.087	0.0694423	0.0694106

24	33.87	-14.2123	19.9956	-0.0193202	0.338884	293.15	293.15	0	307.26	307.26	0.069482	0.0694503

25	34.04	-14.1358	20.0008	-0.0192152	0.344254	293.15	293.15	0	307.434	307.434	0.0695222	0.0694903

26	34.21	-14.1072	19.9904	-0.0191753	0.344802	293.15	293.15	0	307.598	307.598	0.0695627	0.0695308

27	34.38	-14.1105	19.9904	-0.0191787	0.347448	293.15	293.15	0	307.754	307.754	0.0696021	0.0695706

28	34.54	-14.0768	19.9946	-0.0191319	0.349548	293.15	293.15	0	307.927	307.927	0.0696416	0.0696097

29	34.71	-14.0249	20.0008	-0.0190605	0.351961	293.15	293.15	0	308.099	308.099	0.0696809	0.0696492

30	34.88	-13.99	19.9966	-0.019012	0.357203	293.15	293.15	0	308.265	308.265	0.0697208	0.0696901

31	35.05	-13.9834	19.9946	-0.0190021	0.358692	293.15	293.15	0	308.429	308.429	0.0697611	0.0697297

32	35.22	-14.019	20.0008	-0.0190495	0.363109	293.15	293.15	0	308.602	308.602	0.0698	0.0697691

33	35.38	-14.0499	19.9966	-0.0190906	0.367399	293.15	293.15	0	308.773	308.773	0.0698385	0.0698087

34	35.56	-14.1455	19.9998	-0.0192194	0.366751	293.15	293.15	0	308.93	308.93	0.06988	0.0698503

35	35.73	-14.1656	19.9925	-0.0192457	0.368717	293.15	293.15	0	309.088	309.088	0.0699198	0.0698902

36	35.89	-14.1038	19.9904	-0.0191609	0.373841	293.15	293.15	0	309.261	309.261	0.0699587	0.0699293

37	36.06	-14.0079	19.9904	-0.0190296	0.375896	293.15	293.15	0	309.432	309.432	0.0699981	0.0699683

38	36.22	-13.9218	19.9977	-0.0189116	0.382312	293.15	293.15	0	309.59	309.59	0.0700377	0.0700076

39	36.39	-13.8723	19.9987	-0.0188435	0.383563	293.15	293.15	0	309.758	309.758	0.0700776	0.0700474

40	36.56	-13.869	19.9904	-0.0188379	0.386077	293.15	293.15	0	309.927	309.927	0.0701165	0.0700869

41	36.73	-13.8815	19.9977	-0.018854	0.390201	293.15	293.15	0	310.101	310.101	0.0701553	0.0701259

42	36.9	-13.9153	20.0008	-0.0188989	0.393366	293.15	293.15	0	310.259	310.259	0.0701951	0.0701665

43	37.06	-13.9625	20.0008	-0.0189621	0.398699	293.15	293.15	0	310.43	310.43	0.0702338	0.070205

44	37.23	-14.0489	20.0008	-0.0190785	0.401233	293.15	293.15	0	310.595	310.595	0.0702733	0.0702451

45	37.39	-14.0991	20.0008	-0.0191457	0.405227	293.15	293.15	0	310.762	310.762	0.0703117	0.070284

46	37.56	-14.0863	19.9946	-0.0191272	0.409735	293.15	293.15	0	310.934	310.934	0.0703521	0.070324

47	37.73	-14.0518	19.9904	-0.0190795	0.411152	293.15	293.15	0	311.089	311.089	0.0703925	0.0703643

48	37.9	-14.0445	20.0008	-0.0190685	0.414858	293.15	293.15	0	311.253	311.253	0.0704306	0.070403

49	38.06	-14.0287	20.0008	-0.0190462	0.416102	293.15	293.15	0	311.426	311.426	0.0704706	0.0704418

50	38.23	-14.0424	20.0008	-0.0190638	0.421669	293.15	293.15	0	311.599	311.599	0.0705095	0.0704814

51	38.39	-14.0607	20.0008	-0.0190877	0.427255	293.15	293.15	0	311.763	311.763	0.0705477	0.0705197

52	38.56	-14.0167	19.9956	-0.0190269	0.428567	293.15	293.15	0	311.936	311.936	0.0705874	0.0705605

53	38.73	-14.0043	19.9946	-0.0190092	0.433341	293.15	293.15	0	312.084	312.084	0.0706271	0.0705998

54	38.9	-14.0678	20.0008	-0.0190944	0.435281	293.15	293.15	0	312.255	312.255	0.070667	0.0706397

55	39.07	-14.0998	20.0008	-0.0191368	0.43868	293.15	293.15	0	312.421	312.421	0.0707058	0.0706795

56	39.24	-14.0967	19.9966	-0.0191317	0.44118	293.15	293.15	0	312.595	312.595	0.0707448	0.0707189

57	39.4	-14.0978	19.9904	-0.0191322	0.443513	293.15	293.15	0	312.766	312.766	0.0707853	0.0707587

58	39.57	-14.1588	19.9946	-0.019214	0.44869	293.15	293.15	0	312.931	312.931	0.0708239	0.0707981

59	39.74	-14.1829	20.0008	-0.0192456	0.450352	293.15	293.15	0	313.088	313.088	0.0708636	0.0708375

60	39.91	-14.1907	20.0008	-0.0192552	0.454627	293.15	293.15	0	313.259	313.259	0.0709031	0.0708772

61	40.08	-14.1852	20.0008	-0.0192468	0.457354	293.15	293.15	0	313.435	313.435	0.0709428	0.0709174

62	40.24	-14.1944	20.0008	-0.0192584	0.463635	293.15	293.15	0	313.599	313.599	0.0709814	0.0709564

63	40.4	-14.2009	20.0008	-0.0192662	0.467299	293.15	293.15	0	313.768	313.768	0.0710202	0.0709948

64	40.58	-14.2487	19.9987	-0.0193301	0.469244	293.15	293.15	0	313.929	313.929	0.0710597	0.0710356

65	40.74	-14.317	19.9977	-0.0194217	0.470333	293.15	293.15	0	314.093	314.093	0.0710995	0.0710747

66	40.91	-14.3215	20.0008	-0.0194268	0.47646	293.15	293.15	0	314.261	314.261	0.0711387	0.071114

67	41.08	-14.3427	20.0008	-0.0194546	0.479678	293.15	293.15	0	314.431	314.431	0.071178	0.0711539

68	41.25	-14.3831	20.0008	-0.0195084	0.480217	293.15	293.15	0	314.603	314.603	0.0712177	0.0711933

69	41.41	-14.4267	20.0008	-0.0195665	0.482395	293.15	293.15	0	314.752	314.752	0.0712572	0.0712322

70	41.57	-14.3672	20.0008	-0.0194849	0.486467	293.15	293.15	0	314.924	314.924	0.071296	0.0712709

71	41.75	-14.2995	19.9946	-0.0193921	0.492125	293.15	293.15	0	315.097	315.097	0.0713354	0.0713112

72	41.91	-14.2527	19.9966	-0.0193276	0.495922	293.15	293.15	0	315.263	315.263	0.0713743	0.0713505

73	42.08	-14.2193	20.0008	-0.0192813	0.499784	293.15	293.15	0	315.435	315.435	0.0714132	0.07139

74	42.25	-14.1928	20.0008	-0.0192444	0.50336	293.15	293.15	0	315.608	315.608	0.0714534	0.0714299

75	42.41	-14.1519	19.9956	-0.019188	0.504651	293.15	293.15	0	315.755	315.755	0.0714928	0.0714688

76	42.58	-14.1013	20.0008	-0.0191185	0.507544	293.15	293.15	0	315.919	315.919	0.0715314	0.0715073

77	42.74	-14.0958	20.0008	-0.01911	0.513112	293.15	293.15	0	316.094	316.094	0.0715703	0.0715466

78	42.91	-14.0845	20.0008	-0.0190938	0.520035	293.15	293.15	0	316.266	316.266	0.071609	0.0715861

79	43.08	-14.0806	19.9904	-0.0190874	0.521546	293.15	293.15	0	316.43	316.43	0.0716487	0.071626

80	43.25	-14.1373	19.9956	-0.0191634	0.522442	293.15	293.15	0	316.603	316.603	0.0716884	0.0716649

81	43.42	-14.1767	19.9966	-0.0192158	0.524551	293.15	293.15	0	316.758	316.758	0.0717279	0.0717051

82	43.58	-14.2038	19.9998	-0.0192516	0.530351	293.15	293.15	0	316.925	316.925	0.0717671	0.0717444

83	43.75	-14.2498	20.0008	-0.0193129	0.534679	293.15	293.15	0	317.088	317.088	0.0718056	0.0717842

84	43.92	-14.2615	19.9966	-0.0193277	0.535543	293.15	293.15	0	317.269	317.269	0.0718457	0.0718241

85	44.08	-14.2293	19.9998	-0.0192831	0.538251	293.15	293.15	0	317.434	317.434	0.071885	0.0718625

86	44.25	-14.2195	20.0008	-0.0192688	0.542284	293.15	293.15	0	317.6	317.6	0.0719235	0.0719021

87	44.42	-14.2497	20.0008	-0.0193089	0.545718	293.15	293.15	0	317.755	317.755	0.0719643	0.0719412

88	44.59	-14.2285	20.0008	-0.0192791	0.549214	293.15	293.15	0	317.924	317.924	0.0720032	0.0719807

89	44.75	-14.151	20.0008	-0.0191731	0.554585	293.15	293.15	0	318.093	318.093	0.0720412	0.0720202

90	44.92	-14.1145	19.9925	-0.0191226	0.558771	293.15	293.15	0	318.273	318.273	0.0720805	0.0720594

91	45.08	-14.1215	19.9977	-0.0191312	0.563204	293.15	293.15	0	318.432	318.432	0.0721202	0.0720982

92	45.25	-14.0804	20.0008	-0.0190745	0.56538	293.15	293.15	0	318.599	318.599	0.0721594	0.072138

93	45.42	-14.061	20.0008	-0.0190473	0.569197	293.15	293.15	0	318.752	318.752	0.0721973	0.072177

94	45.59	-14.0743	20.0008	-0.0190643	0.573972	293.15	293.15	0	318.925	318.925	0.0722376	0.0722179

95	45.76	-14.106	20.0008	-0.0191063	0.574866	293.15	293.15	0	319.091	319.091	0.0722774	0.0722575

96	45.93	-14.1526	20.0008	-0.0191684	0.57906	293.15	293.15	0	319.272	319.272	0.0723167	0.0722969

97	46.09	-14.1823	20.0008	-0.0192077	0.582033	293.15	293.15	0	319.428	319.428	0.0723563	0.0723353

98	46.26	-14.1408	20.0008	-0.0191506	0.58405	293.15	293.15	0	319.601	319.601	0.0723949	0.0723742

99	46.43	-14.1058	20.0008	-0.0191021	0.589702	293.15	293.15	0	319.765	319.765	0.0724348	0.0724141

100	46.59	-14.1802	19.9966	-0.0192019	0.592606	293.15	293.15	0	319.933	319.933	0.0724731	0.072453

101	46.76	-14.2576	19.9998	-0.0193058	0.597388	293.15	293.15	0	320.094	320.094	0.0725115	0.0724925

102	46.93	-14.2717	20.0008	-0.0193238	0.600689	293.15	293.15	0	320.26	320.26	0.0725513	0.0725321

103	47.09	-14.3136	20.0008	-0.0193796	0.605287	293.15	293.15	0	320.432	320.432	0.0725901	0.0725706

104	47.26	-14.3843	20.0008	-0.0194743	0.607664	293.15	293.15	0	320.604	320.604	0.07263	0.0726111

105	47.43	-14.457	20.0008	-0.0195718	0.610489	293.15	293.15	0	320.754	320.754	0.0726686	0.0726505

106	47.6	-14.4789	20.0008	-0.0196004	0.61349	293.15	293.15	0	320.928	320.928	0.0727091	0.0726905

107	47.76	-14.4501	20.0008	-0.0195604	0.617767	293.15	293.15	0	321.091	321.091	0.0727479	0.0727285

108	47.93	-14.3876	20.0008	-0.0194748	0.625031	293.15	293.15	0	321.261	321.261	0.0727856	0.0727676

109	48.1	-14.3911	19.9977	-0.0194785	0.627779	293.15	293.15	0	321.437	321.437	0.0728252	0.0728077

110	48.27	-14.4129	19.9904	-0.0195071	0.630631	293.15	293.15	0	321.597	321.597	0.0728645	0.072847

111	48.43	-14.4711	19.9925	-0.0195848	0.634418	293.15	293.15	0	321.758	321.758	0.0729038	0.0728867

112	48.6	-14.5498	20.0008	-0.0196904	0.63885	293.15	293.15	0	321.931	321.931	0.0729426	0.0729262

113	48.77	-14.5981	19.9935	-0.0197547	0.642103	293.15	293.15	0	322.096	322.096	0.072982	0.0729655

114	48.94	-14.6176	19.9925	-0.0197801	0.642762	293.15	293.15	0	322.263	322.263	0.0730225	0.0730054

115	49.11	-14.596	20.0008	-0.0197498	0.650151	293.15	293.15	0	322.432	322.432	0.0730611	0.0730452

116	49.27	-14.5827	20.0008	-0.0197309	0.652699	293.15	293.15	0	322.599	322.599	0.0731002	0.0730834

117	49.44	-14.5508	20.0008	-0.0196867	0.655493	293.15	293.15	0	322.755	322.755	0.0731392	0.0731227

118	49.6	-14.5336	20.0008	-0.0196624	0.660249	293.15	293.15	0	322.927	322.927	0.0731773	0.0731614

119	49.77	-14.5474	20.0008	-0.0196801	0.662758	293.15	293.15	0	323.101	323.101	0.0732181	0.0732011

120	49.94	-14.5348	20.0008	-0.019662	0.667762	293.15	293.15	0	323.266	323.266	0.0732565	0.0732406

121	50.1	-14.4887	20.0008	-0.0195987	0.672382	293.15	293.15	0	323.421	323.421	0.0732955	0.0732792

122	50.27	-14.441	20.0008	-0.0195332	0.674049	293.15	293.15	0	323.594	323.594	0.0733349	0.0733186

123	50.44	-14.3994	20.0008	-0.019476	0.683092	293.15	293.15	0	323.759	323.759	0.0733734	0.0733573

124	50.61	-14.4131	20.0008	-0.0194934	0.682284	293.15	293.15	0	323.931	323.931	0.0734137	0.073398

125	50.78	-14.4965	19.9956	-0.0196053	0.684577	293.15	293.15	0	324.095	324.095	0.0734527	0.0734372

126	50.94	-14.5807	19.9904	-0.0197182	0.689021	293.15	293.15	0	324.268	324.268	0.0734911	0.0734767

127	51.12	-14.6321	19.9904	-0.0197866	0.691574	293.15	293.15	0	324.416	324.416	0.0735318	0.0735173

128	51.28	-14.6467	19.9946	-0.0198054	0.696088	293.15	293.15	0	324.59	324.59	0.0735701	0.0735553

129	51.45	-14.6158	20.0008	-0.0197626	0.698733	293.15	293.15	0	324.76	324.76	0.0736095	0.0735946

130	51.61	-14.6214	20.0008	-0.0197691	0.701433	293.15	293.15	0	324.926	324.926	0.0736484	0.0736342

131	51.78	-14.6195	20.0008	-0.0197656	0.707305	293.15	293.15	0	325.099	325.099	0.0736875	0.0736725

132	51.95	-14.6344	20.0008	-0.0197848	0.711591	293.15	293.15	0	325.271	325.271	0.0737257	0.0737123

133	52.11	-14.6737	20.0008	-0.0198369	0.714886	293.15	293.15	0	325.437	325.437	0.0737643	0.0737508

134	52.29	-14.7572	20.0008	-0.0199487	0.717935	293.15	293.15	0	325.603	325.603	0.0738048	0.0737919

135	52.44	-14.7983	20.0008	-0.0200033	0.725934	293.15	293.15	0	325.757	325.757	0.0738422	0.0738286

136	52.61	-14.7589	19.9977	-0.0199491	0.726789	293.15	293.15	0	325.927	325.927	0.0738824	0.0738682

137	52.78	-14.7171	19.9904	-0.0198915	0.731287	293.15	293.15	0	326.095	326.095	0.0739216	0.0739076

138	52.94	-14.7031	19.9987	-0.0198716	0.735381	293.15	293.15	0	326.268	326.268	0.0739598	0.0739458

139	53.11	-14.6802	20.0008	-0.0198396	0.739468	293.15	293.15	0	326.419	326.419	0.0739994	0.0739861

140	53.28	-14.6411	19.9935	-0.0197858	0.743391	293.15	293.15	0	326.589	326.589	0.0740391	0.0740252

141	53.45	-14.6139	19.9977	-0.019748	0.746803	293.15	293.15	0	326.762	326.762	0.0740776	0.0740641

142	53.61	-14.6758	20.0008	-0.0198307	0.750104	293.15	293.15	0	326.93	326.93	0.074116	0.0741031

143	53.78	-14.7954	20.0008	-0.0199913	0.757269	293.15	293.15	0	327.099	327.099	0.0741551	0.0741417

144	53.95	-14.8225	20.0008	-0.0200268	0.759729	293.15	293.15	0	327.265	327.265	0.0741945	0.0741814

145	54.12	-14.8608	20.0008	-0.0200776	0.761862	293.15	293.15	0	327.422	327.422	0.0742336	0.0742217

146	54.29	-14.9279	19.9946	-0.0201673	0.764781	293.15	293.15	0	327.593	327.593	0.0742736	0.0742614

147	54.45	-15.0178	19.9966	-0.0202877	0.768486	293.15	293.15	0	327.757	327.757	0.0743123	0.0743004

148	54.62	-15.0769	20.0008	-0.0203665	0.775585	293.15	293.15	0	327.931	327.931	0.0743507	0.0743395

149	54.79	-15.1045	20.0008	-0.0204027	0.778993	293.15	293.15	0	328.096	328.096	0.0743903	0.074379

150	54.95	-15.1444	19.9998	-0.0204556	0.784334	293.15	293.15	0	328.269	328.269	0.0744285	0.0744181

151	55.12	-15.2048	19.9904	-0.0205361	0.789316	293.15	293.15	0	328.425	328.425	0.0744678	0.0744572

152	55.29	-15.3146	19.9956	-0.0206833	0.793548	293.15	293.15	0	328.589	328.589	0.0745072	0.0744963

153	55.46	-15.469	19.9956	-0.0208908	0.79592	293.15	293.15	0	328.762	328.762	0.0745456	0.0745357

154	55.62	-15.5689	20.0008	-0.0210247	0.799016	293.15	293.15	0	328.935	328.935	0.0745847	0.0745751

155	55.79	-15.6313	20.0008	-0.0211079	0.805314	293.15	293.15	0	329.099	329.099	0.0746236	0.0746139

156	55.96	-15.6772	19.9956	-0.0211688	0.810316	293.15	293.15	0	329.272	329.272	0.0746622	0.0746528

157	56.12	-15.7771	19.9998	-0.0213026	0.814685	293.15	293.15	0	329.419	329.419	0.0747003	0.0746914

158	56.29	-15.8937	20.0008	-0.0214589	0.817433	293.15	293.15	0	329.591	329.591	0.0747394	0.0747309

159	56.46	-16.1455	20.0008	-0.0217978	0.822423	293.15	293.15	0	329.757	329.757	0.0747796	0.0747716

160	56.63	-16.3903	20.0008	-0.0221272	0.82765	293.15	293.15	0	329.928	329.928	0.0748187	0.0748111

161	56.8	-16.5685	20.0008	-0.0223666	0.832619	293.15	293.15	0	330.096	330.096	0.0748566	0.0748498

162	56.96	-16.7841	19.9925	-0.0226565	0.837157	293.15	293.15	0	330.26	330.26	0.0748956	0.0748893

163	57.13	-17.0944	19.9904	-0.0230743	0.843053	293.15	293.15	0	330.43	330.43	0.0749335	0.0749277

164	57.29	-17.4658	19.9904	-0.0235744	0.851099	293.15	293.15	0	330.597	330.597	0.0749715	0.0749662

165	57.46	-17.8671	19.9987	-0.0241148	0.857669	293.15	293.15	0	330.771	330.771	0.0750099	0.0750053

166	57.63	-18.3407	20.0008	-0.0247527	0.863504	293.15	293.15	0	330.931	330.931	0.0750483	0.0750447

167	57.8	-18.9414	20.0008	-0.0255621	0.870617	293.15	293.15	0	331.092	331.092	0.0750863	0.0750841

168	57.96	-19.6498	20.0008	-0.0265168	0.879968	293.15	293.15	0	331.264	331.264	0.0751234	0.075123

169	58.13	-20.4833	20.0008	-0.0276401	0.888977	293.15	293.15	0	331.43	331.43	0.0751605	0.0751621

170	58.29	-21.4917	20.0008	-0.0289995	0.89787	293.15	293.15	0	331.596	331.596	0.0751968	0.0752009

171	58.46	-22.7219	20.0008	-0.0306579	0.911772	293.15	293.15	0	331.766	331.766	0.0752336	0.0752398

172	58.62	-24.174	19.9935	-0.0326156	0.923785	293.15	293.15	0	331.932	331.932	0.0752695	0.0752783

173	58.79	-25.8984	19.9914	-0.0349403	0.937431	293.15	293.15	0	332.087	332.087	0.0753041	0.0753166

174	58.95	-28.0187	19.9946	-0.037799	0.953963	293.15	293.15	0	332.253	332.253	0.0753391	0.0753554

175	59.12	-30.5549	19.9914	-0.0412185	0.975294	293.15	293.15	0	332.425	332.425	0.0753725	0.0753934

176	59.28	-33.4349	20.0008	-0.0451014	0.997555	293.15	293.15	0	332.597	332.597	0.0754058	0.0754317

177	59.44	-36.6983	20.0008	-0.049501	1.02046	293.15	293.15	0	332.763	332.763	0.0754384	0.0754701

178	59.61	-40.4506	20.0008	-0.0545596	1.04399	293.15	293.15	0	332.926	332.926	0.0754709	0.0755085

179	59.78	-44.6005	19.9904	-0.060154	1.07288	293.15	293.15	0	333.092	333.092	0.0755035	0.0755483

180	59.94	-49.0288	19.9956	-0.0661232	1.09874	293.15	293.15	0	333.255	333.255	0.075535	0.075587

181	60.11	-53.7269	20.0008	-0.0724556	1.12347	293.15	293.15	0	333.42	333.42	0.0755689	0.0756268

182	60.29	-58.3471	20.0008	-0.0786822	1.15121	293.15	293.15	0	333.601	333.601	0.0756034	0.0756679

183	60.47	-62.8069	19.9956	-0.0846917	1.17699	293.15	293.15	0	333.765	333.765	0.0756394	0.0757104

184	60.66	-67.0691	19.9956	-0.0904339	1.19468	293.15	293.15	0	333.938	333.938	0.0756786	0.075754

185	60.85	-70.9512	19.9904	-0.0956628	1.21203	293.15	293.15	0	334.103	334.103	0.0757179	0.0757986

186	61.04	-74.3972	19.9946	-0.100303	1.22402	293.15	293.15	0	334.267	334.267	0.0757602	0.075843

187	61.23	-77.4104	20.0008	-0.10436	1.23832	293.15	293.15	0	334.424	334.424	0.0758016	0.0758891

188	61.43	-80.0666	20.0008	-0.107934	1.24683	293.15	293.15	0	334.597	334.597	0.0758451	0.0759351

189	61.63	-82.4469	19.9966	-0.111136	1.25389	293.15	293.15	0	334.761	334.761	0.0758892	0.0759811

190	61.82	-84.4498	19.9904	-0.113829	1.2596	293.15	293.15	0	334.932	334.932	0.0759331	0.0760265

191	62.02	-86.0158	19.9998	-0.115933	1.26805	293.15	293.15	0	335.098	335.098	0.0759774	0.0760722

192	62.21	-87.2141	20.0008	-0.117541	1.27235	293.15	293.15	0	335.264	335.264	0.0760223	0.0761176

193	62.4	-88.0583	20.0008	-0.118672	1.27375	293.15	293.15	0	335.425	335.425	0.076066	0.0761624

194	62.6	-88.6728	20.0008	-0.119493	1.27496	293.15	293.15	0	335.593	335.593	0.0761119	0.0762079

195	62.79	-88.993	20.0008	-0.119918	1.27543	293.15	293.15	0	335.766	335.766	0.0761568	0.0762525

196	62.98	-89.0536	20.0008	-0.119993	1.27255	293.15	293.15	0	335.935	335.935	0.0762018	0.0762967

197	63.16	-88.8571	20.0008	-0.119721	1.27335	293.15	293.15	0	336.102	336.102	0.0762457	0.0763405

198	63.35	-88.5331	20.0008	-0.119278	1.27129	293.15	293.15	0	336.269	336.269	0.0762884	0.0763841

199	63.53	-88.0783	20.0008	-0.118659	1.2711	293.15	293.15	0	336.423	336.423	0.0763331	0.076427

200	63.71	-87.4784	20.0008	-0.117844	1.26731	293.15	293.15	0	336.591	336.591	0.0763765	0.0764691

201	63.89	-86.7495	20.0008	-0.116856	1.26491	293.15	293.15	0	336.761	336.761	0.0764189	0.0765111

202	64.07	-85.9263	19.9935	-0.115741	1.26376	293.15	293.15	0	336.934	336.934	0.0764609	0.076552

203	64.24	-85.0711	19.9977	-0.114583	1.26341	293.15	293.15	0	337.101	337.101	0.0765025	0.0765925

204	64.41	-84.1608	20.0008	-0.113351	1.25941	293.15	293.15	0	337.262	337.262	0.0765443	0.0766323

205	64.58	-83.1732	20.0008	-0.112015	1.25659	293.15	293.15	0	337.427	337.427	0.0765857	0.0766725

206	64.76	-82.0102	20.0008	-0.110443	1.25331	293.15	293.15	0	337.592	337.592	0.0766275	0.0767127

207	64.93	-80.7383	19.9946	-0.108724	1.25194	293.15	293.15	0	337.757	337.757	0.076669	0.0767521

208	65.09	-79.449	19.9966	-0.106983	1.25175	293.15	293.15	0	337.938	337.938	0.0767091	0.0767909

209	65.26	-78.1045	20.0008	-0.105167	1.24861	293.15	293.15	0	338.104	338.104	0.0767497	0.0768294

210	65.42	-76.773	20.0008	-0.103369	1.24603	293.15	293.15	0	338.26	338.26	0.0767905	0.0768677

211	65.59	-75.3832	20.0008	-0.101493	1.24538	293.15	293.15	0	338.423	338.423	0.0768303	0.0769065

212	65.75	-73.9566	20.0008	-0.0995671	1.24028	293.15	293.15	0	338.596	338.596	0.0768714	0.0769455

213	65.91	-72.4856	20.0008	-0.0975819	1.23525	293.15	293.15	0	338.76	338.76	0.0769114	0.0769833

214	66.08	-70.7879	19.9956	-0.0952917	1.23282	293.15	293.15	0	338.925	338.925	0.0769525	0.0770219

215	66.24	-68.874	20.0008	-0.0927107	1.22817	293.15	293.15	0	339.098	339.098	0.0769931	0.0770602

216	66.41	-66.6276	20.0008	-0.0896822	1.21358	293.15	293.15	0	339.272	339.272	0.0770375	0.0770989

217	66.58	-64.0534	20.0008	-0.0862129	1.2018	293.15	293.15	0	339.418	339.418	0.0770812	0.0771387

218	66.74	-61.2421	20.0008	-0.082425	1.1883	293.15	293.15	0	339.599	339.599	0.0771233	0.077177

219	66.91	-57.6828	20.0008	-0.0776306	1.17294	293.15	293.15	0	339.765	339.765	0.0771705	0.0772167

220	67.08	-53.2407	20.0008	-0.0716487	1.15302	293.15	293.15	0	339.927	339.927	0.0772178	0.0772565

221	67.26	-48.1115	20.0008	-0.0647424	1.12358	293.15	293.15	0	340.095	340.095	0.0772672	0.0772984

222	67.43	-42.8968	20.0008	-0.0577223	1.1017	293.15	293.15	0	340.269	340.269	0.077313	0.0773377

223	67.59	-38.0113	19.9977	-0.0511458	1.08651	293.15	293.15	0	340.433	340.433	0.0773552	0.0773743

224	67.74	-33.5339	19.9987	-0.0451192	1.07454	293.15	293.15	0	340.602	340.602	0.077395	0.0774097

225	67.88	-29.6059	19.9925	-0.0398324	1.06434	293.15	293.15	0	340.761	340.761	0.0774328	0.0774432

226	68.03	-26.1545	19.9946	-0.0351874	1.05542	293.15	293.15	0	340.926	340.926	0.0774696	0.0774766

227	68.17	-23.1103	20.0039	-0.0310905	1.05485	293.15	293.15	0	341.09	341.09	0.0775047	0.077509

228	68.3	-20.4396	20.0008	-0.0274964	1.05296	293.15	293.15	0	341.258	341.258	0.0775384	0.0775397

229	68.43	-18.0672	20.0008	-0.0243039	1.05295	293.15	293.15	0	341.428	341.428	0.0775715	0.0775712

230	68.57	-16.1944	20.0008	-0.0217839	1.05572	293.15	293.15	0	341.6	341.6	0.0776046	0.0776028

231	68.71	-14.8737	20.0008	-0.0200065	1.06176	293.15	293.15	0	341.751	341.751	0.0776371	0.0776347

232	68.84	-13.8556	20.0008	-0.0186363	1.06613	293.15	293.15	0	341.922	341.922	0.0776695	0.0776666

233	68.98	-13.0555	19.9946	-0.0175593	1.07161	293.15	293.15	0	342.095	342.095	0.0777024	0.0776994

234	69.12	-12.4286	19.9966	-0.0167155	1.08181	293.15	293.15	0	342.261	342.261	0.0777355	0.077732

235	69.27	-12.0526	20.0008	-0.016209	1.08883	293.15	293.15	0	342.432	342.432	0.0777688	0.0777659

236	69.41	-11.8228	20.0008	-0.0158994	1.09851	293.15	293.15	0	342.605	342.605	0.0778027	0.0777996

237	69.56	-11.7615	20.0008	-0.0158162	1.1033	293.15	293.15	0	342.752	342.752	0.0778377	0.0778343

238	69.71	-11.763	20.0008	-0.0158175	1.10962	293.15	293.15	0	342.926	342.926	0.077872	0.0778697

239	69.87	-11.7782	19.9956	-0.0158371	1.12103	293.15	293.15	0	343.09	343.09	0.077908	0.0779059

240	70.03	-11.8642	19.9904	-0.0159521	1.12614	293.15	293.15	0	343.263	343.263	0.0779438	0.0779426

241	70.19	-11.9923	19.9956	-0.0161235	1.13111	293.15	293.15	0	343.436	343.436	0.0779812	0.0779799

242	70.34	-12.0835	19.9956	-0.0162454	1.14018	293.15	293.15	0	343.601	343.601	0.0780183	0.0780166

243	70.5	-12.1812	19.9904	-0.0163759	1.14578	293.15	293.15	0	343.755	343.755	0.0780551	0.078053

244	70.67	-12.2897	19.9904	-0.016521	1.1503	293.15	293.15	0	343.921	343.921	0.0780923	0.0780918

245	70.83	-12.3744	19.9946	-0.0166341	1.15528	293.15	293.15	0	344.085	344.085	0.0781302	0.0781296

246	70.99	-12.4575	19.9914	-0.0167448	1.15915	293.15	293.15	0	344.266	344.266	0.0781681	0.0781677

247	71.16	-12.5374	19.9946	-0.0168515	1.16675	293.15	293.15	0	344.431	344.431	0.0782067	0.0782061

248	71.32	-12.6266	20.0008	-0.0169705	1.17216	293.15	293.15	0	344.605	344.605	0.0782442	0.0782449

249	71.49	-12.6272	20.0008	-0.0169705	1.17466	293.15	293.15	0	344.769	344.769	0.0782837	0.0782841

250	71.66	-12.5786	20.0008	-0.0169043	1.17995	293.15	293.15	0	344.931	344.931	0.0783224	0.0783229

251	71.82	-12.6993	20.0008	-0.0170657	1.18722	293.15	293.15	0	345.09	345.09	0.0783601	0.0783612

252	71.99	-12.8326	19.9925	-0.017244	1.1953	293.15	293.15	0	345.263	345.263	0.0783983	0.0784004

253	72.16	-12.8864	19.9935	-0.0173154	1.19562	293.15	293.15	0	345.427	345.427	0.0784383	0.0784399

254	72.33	-12.9081	20.0008	-0.0173435	1.19788	293.15	293.15	0	345.596	345.596	0.078478	0.0784801

255	72.5	-12.9791	20.0008	-0.0174381	1.20572	293.15	293.15	0	345.764	345.764	0.078516	0.0785184

256	72.66	-13.064	19.9987	-0.0175513	1.21048	293.15	293.15	0	345.93	345.93	0.0785553	0.0785573

257	72.83	-13.1059	19.9977	-0.0176067	1.21269	293.15	293.15	0	346.088	346.088	0.0785945	0.078597

258	73	-13.1394	20.0008	-0.0176508	1.21577	293.15	293.15	0	346.258	346.258	0.0786336	0.0786352

259	73.17	-13.1137	20.0008	-0.0176153	1.22176	293.15	293.15	0	346.432	346.432	0.0786731	0.078675

260	73.33	-13.0459	19.9935	-0.0175234	1.22546	293.15	293.15	0	346.6	346.6	0.0787113	0.0787132

261	73.5	-12.9619	19.9977	-0.0174097	1.22925	293.15	293.15	0	346.768	346.768	0.0787495	0.0787514

262	73.67	-12.8716	20.0008	-0.0172876	1.23566	293.15	293.15	0	346.934	346.934	0.0787888	0.0787909

263	73.83	-12.8241	20.0008	-0.0172229	1.23889	293.15	293.15	0	347.089	347.089	0.0788272	0.0788297

264	74	-12.7125	20.0008	-0.0170721	1.24363	293.15	293.15	0	347.255	347.255	0.0788659	0.0788683

265	74.17	-12.8116	20.0008	-0.0172043	1.25105	293.15	293.15	0	347.426	347.426	0.0789032	0.078907

266	74.34	-12.9335	20.0008	-0.0173672	1.2546	293.15	293.15	0	347.6	347.6	0.0789428	0.0789466

267	74.51	-12.9884	20.0008	-0.01744	1.25913	293.15	293.15	0	347.765	347.765	0.0789826	0.078987

268	74.68	-13.0134	20.0008	-0.0174727	1.26425	293.15	293.15	0	347.928	347.928	0.0790205	0.0790259

269	74.84	-13.0065	20.0008	-0.0174625	1.26652	293.15	293.15	0	348.085	348.085	0.07906	0.0790639

270	75.01	-12.9694	20.0008	-0.0174118	1.27378	293.15	293.15	0	348.258	348.258	0.079098	0.0791023

271	75.17	-12.9156	19.9904	-0.0173387	1.27674	293.15	293.15	0	348.431	348.431	0.0791373	0.0791417

272	75.34	-12.8734	19.9956	-0.0172812	1.27887	293.15	293.15	0	348.595	348.595	0.0791768	0.0791812

273	75.51	-12.8689	20.0008	-0.0172743	1.28277	293.15	293.15	0	348.768	348.768	0.0792151	0.07922

274	75.68	-12.8905	20.0008	-0.0173025	1.28974	293.15	293.15	0	348.932	348.932	0.0792541	0.079259

275	75.85	-12.8485	20.0008	-0.0172452	1.29367	293.15	293.15	0	349.096	349.096	0.079293	0.0792981

276	76.01	-12.8474	20.0008	-0.0172429	1.29685	293.15	293.15	0	349.269	349.269	0.0793315	0.079337

277	76.18	-12.8379	19.9914	-0.0172293	1.2996	293.15	293.15	0	349.427	349.427	0.0793704	0.0793756

278	76.35	-12.7938	19.9946	-0.0171692	1.30645	293.15	293.15	0	349.599	349.599	0.079409	0.0794138

279	76.51	-12.6743	20.0008	-0.017008	1.30959	293.15	293.15	0	349.764	349.764	0.0794478	0.0794529

280	76.68	-12.6392	20.0008	-0.01696	1.31625	293.15	293.15	0	349.926	349.926	0.0794858	0.0794918

281	76.85	-12.6548	20.0008	-0.01698	1.31973	293.15	293.15	0	350.094	350.094	0.0795247	0.0795313

282	77.01	-12.6974	19.9925	-0.0170363	1.32382	293.15	293.15	0	350.264	350.264	0.0795638	0.0795694

283	77.18	-12.7305	19.9904	-0.0170799	1.33059	293.15	293.15	0	350.423	350.423	0.0796025	0.0796087

284	77.35	-12.7727	19.9925	-0.0171357	1.33236	293.15	293.15	0	350.591	350.591	0.0796418	0.0796483

285	77.52	-12.7448	20.0008	-0.0170974	1.33646	293.15	293.15	0	350.761	350.761	0.0796797	0.0796859

286	77.69	-12.6179	20.0008	-0.0169262	1.34063	293.15	293.15	0	350.934	350.934	0.0797195	0.0797264

287	77.85	-12.5086	20.0008	-0.0167789	1.34651	293.15	293.15	0	351.098	351.098	0.0797576	0.0797639

288	78.01	-12.4541	20.0008	-0.0167049	1.35067	293.15	293.15	0	351.265	351.265	0.0797959	0.0798018

289	78.19	-12.4939	20.0008	-0.0167574	1.35379	293.15	293.15	0	351.419	351.419	0.0798346	0.0798418

290	78.35	-12.5322	20.0008	-0.016808	1.35801	293.15	293.15	0	351.593	351.593	0.079874	0.079881

291	78.52	-12.5808	20.0008	-0.0168722	1.36484	293.15	293.15	0	351.758	351.758	0.0799119	0.0799189

292	78.69	-12.6376	19.9946	-0.0169477	1.36637	293.15	293.15	0	351.929	351.929	0.0799515	0.0799584

293	78.85	-12.6251	19.9904	-0.01693	1.37372	293.15	293.15	0	352.102	352.102	0.0799899	0.0799961

294	79.02	-12.5609	19.9966	-0.0168431	1.3797	293.15	293.15	0	352.26	352.26	0.0800278	0.0800351

295	79.18	-12.4711	20.0008	-0.0167219	1.3857	293.15	293.15	0	352.423	352.423	0.0800663	0.0800726

296	79.35	-12.3699	19.9904	-0.0165853	1.3895	293.15	293.15	0	352.596	352.596	0.0801051	0.0801125

297	79.52	-12.3013	19.9956	-0.0164925	1.39411	293.15	293.15	0	352.761	352.761	0.0801437	0.0801518

298	79.69	-12.2868	19.9956	-0.0164723	1.39937	293.15	293.15	0	352.926	352.926	0.0801829	0.0801899

299	79.85	-12.3709	20.0008	-0.0165841	1.40432	293.15	293.15	0	353.097	353.097	0.0802212	0.0802291

300	80.02	-12.4308	20.0008	-0.0166635	1.40674	293.15	293.15	0	353.262	353.262	0.08026	0.0802683

301	80.19	-12.4776	20.0008	-0.0167255	1.40892	293.15	293.15	0	353.418	353.418	0.0802991	0.0803069

302	80.36	-12.4584	20.0008	-0.0166988	1.41363	293.15	293.15	0	353.591	353.591	0.080337	0.0803462

303	80.52	-12.484	20.0008	-0.0167324	1.42087	293.15	293.15	0	353.763	353.763	0.0803758	0.0803849

304	80.69	-12.4985	20.0008	-0.0167509	1.42389	293.15	293.15	0	353.929	353.929	0.0804151	0.0804242

305	80.86	-12.4753	20.0008	-0.0167191	1.42893	293.15	293.15	0	354.102	354.102	0.0804533	0.080462

306	81.03	-12.459	20.0008	-0.0166963	1.43359	293.15	293.15	0	354.264	354.264	0.0804917	0.0805016

307	81.2	-12.5512	20.0008	-0.016819	1.44033	293.15	293.15	0	354.423	354.423	0.0805309	0.0805409

308	81.36	-12.5877	19.9925	-0.0168671	1.44563	293.15	293.15	0	354.596	354.596	0.0805685	0.0805788

309	81.53	-12.5751	19.9935	-0.0168493	1.44696	293.15	293.15	0	354.761	354.761	0.0806087	0.080618

310	81.7	-12.5646	20.0008	-0.0168345	1.45255	293.15	293.15	0	354.93	354.93	0.0806462	0.0806567

311	81.86	-12.5615	20.0008	-0.0168295	1.45684	293.15	293.15	0	355.098	355.098	0.080686	0.0806952

312	82.03	-12.6378	20.0008	-0.0169308	1.46486	293.15	293.15	0	355.264	355.264	0.0807241	0.0807341

313	82.2	-12.6693	19.9935	-0.0169722	1.46678	293.15	293.15	0	355.422	355.422	0.0807624	0.0807728

314	82.37	-12.6163	19.9904	-0.0169003	1.47063	293.15	293.15	0	355.591	355.591	0.0808017	0.0808127

315	82.53	-12.5407	19.9925	-0.0167982	1.47517	293.15	293.15	0	355.765	355.765	0.0808411	0.0808513

316	82.7	-12.52	20.0008	-0.0167696	1.4795	293.15	293.15	0	355.932	355.932	0.0808794	0.0808901

317	82.87	-12.4615	20.0008	-0.0166904	1.48442	293.15	293.15	0	356.102	356.102	0.0809166	0.080928

318	83.03	-12.3539	20.0008	-0.0165455	1.4893	293.15	293.15	0	356.268	356.268	0.0809559	0.0809667

319	83.2	-12.2834	20.0008	-0.0164503	1.49417	293.15	293.15	0	356.423	356.423	0.0809949	0.081006

320	83.37	-12.3012	20.0008	-0.0164733	1.49789	293.15	293.15	0	356.589	356.589	0.0810329	0.0810439

321	83.53	-12.2985	20.0008	-0.0164688	1.50289	293.15	293.15	0	356.76	356.76	0.0810714	0.0810828

322	83.7	-12.2302	20.0008	-0.0163765	1.51035	293.15	293.15	0	356.934	356.934	0.0811104	0.0811213

323	83.87	-12.2437	20.0008	-0.0163938	1.51573	293.15	293.15	0	357.099	357.099	0.0811479	0.0811605

324	84.04	-12.2672	20.0008	-0.0164245	1.51777	293.15	293.15	0	357.261	357.261	0.0811881	0.0811995

325	84.2	-12.2615	20.0008	-0.016416	1.5219	293.15	293.15	0	357.419	357.419	0.0812264	0.0812383

326	84.37	-12.2315	20.0008	-0.016375	1.53113	293.15	293.15	0	357.593	357.593	0.0812648	0.0812763

327	84.53	-12.2447	19.9956	-0.0163918	1.53605	293.15	293.15	0	357.764	357.764	0.0813025	0.081315

328	84.7	-12.2405	19.9956	-0.0163854	1.53901	293.15	293.15	0	357.928	357.928	0.0813412	0.0813533

329	84.87	-12.3105	20.0008	-0.0164782	1.5418	293.15	293.15	0	358.102	358.102	0.08138	0.0813933

330	85.04	-12.4205	20.0008	-0.0166247	1.547	293.15	293.15	0	358.266	358.266	0.0814194	0.0814319

331	85.21	-12.4621	20.0008	-0.0166796	1.55392	293.15	293.15	0	358.438	358.438	0.0814574	0.0814706

332	85.37	-12.4673	20.0008	-0.0166857	1.55972	293.15	293.15	0	358.603	358.603	0.0814959	0.0815091

333	85.54	-12.4573	20.0008	-0.0166713	1.56047	293.15	293.15	0	358.759	358.759	0.0815343	0.0815482

334	85.71	-12.4693	20.0008	-0.0166865	1.5641	293.15	293.15	0	358.932	358.932	0.0815744	0.0815877

335	85.88	-12.5315	20.0008	-0.016769	1.5721	293.15	293.15	0	359.099	359.099	0.0816123	0.0816265

336	86.05	-12.5298	20.0008	-0.0167659	1.57687	293.15	293.15	0	359.268	359.268	0.0816504	0.0816651

337	86.21	-12.5516	20.0008	-0.0167942	1.58021	293.15	293.15	0	359.419	359.419	0.0816898	0.0817036

338	86.38	-12.6091	20.0008	-0.0168703	1.5845	293.15	293.15	0	359.592	359.592	0.0817277	0.0817418

339	86.55	-12.6114	20.0008	-0.0168725	1.59156	293.15	293.15	0	359.761	359.761	0.081767	0.0817813

340	86.71	-12.5739	19.9998	-0.0168216	1.59483	293.15	293.15	0	359.924	359.924	0.0818051	0.0818201

341	86.88	-12.5359	19.9904	-0.0167698	1.60116	293.15	293.15	0	360.096	360.096	0.0818432	0.0818582

342	87.05	-12.5436	19.9966	-0.0167793	1.60563	293.15	293.15	0	360.269	360.269	0.081882	0.0818966

343	87.22	-12.6023	20.0008	-0.016857	1.60897	293.15	293.15	0	360.434	360.434	0.0819203	0.0819359

344	87.38	-12.6125	20.0008	-0.0168698	1.61561	293.15	293.15	0	360.59	360.59	0.0819595	0.0819748

345	87.55	-12.5557	20.0008	-0.0167929	1.61798	293.15	293.15	0	360.763	360.763	0.0819982	0.0820133

346	87.72	-12.5566	20.0008	-0.0167933	1.62564	293.15	293.15	0	360.927	360.927	0.0820358	0.0820524

347	87.88	-12.5522	20.0008	-0.0167866	1.63144	293.15	293.15	0	361.1	361.1	0.0820753	0.0820909

348	88.05	-12.5243	20.0008	-0.0167484	1.63504	293.15	293.15	0	361.264	361.264	0.0821132	0.0821289

349	88.22	-12.4871	20.0008	-0.0166978	1.63865	293.15	293.15	0	361.421	361.421	0.0821521	0.0821673

350	88.38	-12.4628	19.9966	-0.0166646	1.64285	293.15	293.15	0	361.601	361.601	0.0821902	0.0822062

351	88.55	-12.4724	19.9904	-0.0166765	1.6465	293.15	293.15	0	361.768	361.768	0.082229	0.0822445

352	88.72	-12.4354	19.9998	-0.0166262	1.65557	293.15	293.15	0	361.932	361.932	0.0822677	0.0822832

353	88.88	-12.3704	20.0008	-0.0165385	1.65912	293.15	293.15	0	362.089	362.089	0.0823056	0.0823218

354	89.05	-12.2968	19.9977	-0.0164393	1.66373	293.15	293.15	0	362.258	362.258	0.0823439	0.0823605

355	89.22	-12.2233	19.9987	-0.0163402	1.67034	293.15	293.15	0	362.425	362.425	0.0823825	0.0823988

356	89.39	-12.1779	19.9977	-0.0162786	1.67429	293.15	293.15	0	362.599	362.599	0.0824222	0.0824384

357	89.55	-12.2521	19.9904	-0.016377	1.67963	293.15	293.15	0	362.768	362.768	0.0824602	0.0824767

358	89.72	-12.3674	19.9904	-0.0165303	1.6831	293.15	293.15	0	362.937	362.937	0.0824994	0.0825154

359	89.89	-12.4284	19.9925	-0.0166111	1.68739	293.15	293.15	0	363.083	363.083	0.0825385	0.0825553

360	90.05	-12.4857	20.0008	-0.0166867	1.69427	293.15	293.15	0	363.26	363.26	0.0825761	0.0825924

361	90.22	-12.4918	19.9935	-0.0166941	1.69823	293.15	293.15	0	363.43	363.43	0.0826143	0.0826314

362	90.39	-12.4388	19.9925	-0.0166224	1.70124	293.15	293.15	0	363.594	363.594	0.0826537	0.0826708

363	90.55	-12.3592	20.0008	-0.0165152	1.70687	293.15	293.15	0	363.767	363.767	0.0826911	0.0827085

364	90.72	-12.2715	20.0008	-0.0163973	1.71352	293.15	293.15	0	363.935	363.935	0.0827297	0.082747

365	90.89	-12.1621	20.0008	-0.0162502	1.71646	293.15	293.15	0	364.089	364.089	0.0827684	0.0827858

366	91.06	-12.1237	20.0008	-0.0161981	1.72319	293.15	293.15	0	364.261	364.261	0.0828066	0.0828243

367	91.22	-12.1875	19.9946	-0.0162826	1.72747	293.15	293.15	0	364.425	364.425	0.0828451	0.0828624

368	91.39	-12.1912	19.9904	-0.0162866	1.73417	293.15	293.15	0	364.591	364.591	0.0828831	0.0829013

369	91.56	-12.1696	19.9966	-0.016257	1.73864	293.15	293.15	0	364.763	364.763	0.0829218	0.0829402

370	91.73	-12.1668	20.0008	-0.0162523	1.74263	293.15	293.15	0	364.936	364.936	0.0829606	0.0829797

371	91.89	-12.1978	20.0008	-0.0162931	1.75006	293.15	293.15	0	365.084	365.084	0.0829982	0.0830174

372	92.06	-12.2323	20.0008	-0.0163383	1.75612	293.15	293.15	0	365.256	365.256	0.0830373	0.0830559

373	92.23	-12.2526	20.0008	-0.0163645	1.76023	293.15	293.15	0	365.43	365.43	0.0830757	0.0830951

374	92.39	-12.2865	20.0008	-0.016409	1.76246	293.15	293.15	0	365.594	365.594	0.0831149	0.0831338

375	92.56	-12.2435	20.0008	-0.0163508	1.7707	293.15	293.15	0	365.767	365.767	0.0831533	0.0831731

376	92.73	-12.2187	20.0008	-0.0163169	1.77413	293.15	293.15	0	365.94	365.94	0.0831922	0.0832118

377	92.9	-12.2426	20.0008	-0.0163479	1.77803	293.15	293.15	0	366.105	366.105	0.0832303	0.08325

378	93.07	-12.272	20.0008	-0.0163864	1.78223	293.15	293.15	0	366.27	366.27	0.0832683	0.0832887

379	93.23	-12.1997	20.0008	-0.016289	1.78443	293.15	293.15	0	366.425	366.425	0.0833077	0.0833272

380	93.4	-12.1263	20.0008	-0.0161902	1.79403	293.15	293.15	0	366.597	366.597	0.0833455	0.0833652

381	93.56	-12.1758	20.0008	-0.0162555	1.79867	293.15	293.15	0	366.763	366.763	0.0833835	0.0834033

382	93.73	-12.2547	19.9914	-0.01636	1.80158	293.15	293.15	0	366.935	366.935	0.0834224	0.0834421

383	93.9	-12.3127	19.9998	-0.0164366	1.80939	293.15	293.15	0	367.099	367.099	0.0834604	0.0834809

384	94.06	-12.3045	20.0008	-0.0164249	1.81435	293.15	293.15	0	367.262	367.262	0.0834989	0.0835195

385	94.23	-12.2169	19.9925	-0.0163071	1.81827	293.15	293.15	0	367.42	367.42	0.0835369	0.0835574

386	94.4	-12.1428	19.9987	-0.0162074	1.82505	293.15	293.15	0	367.594	367.594	0.0835753	0.0835962

387	94.56	-12.1361	19.9977	-0.0161976	1.83165	293.15	293.15	0	367.766	367.766	0.0836137	0.0836349

388	94.73	-12.1939	19.9904	-0.0162739	1.83571	293.15	293.15	0	367.931	367.931	0.0836526	0.0836742

389	94.91	-12.2903	19.9987	-0.0164018	1.83965	293.15	293.15	0	368.104	368.104	0.0836923	0.0837139

390	95.07	-12.3148	19.9977	-0.0164337	1.84371	293.15	293.15	0	368.268	368.268	0.0837304	0.0837516

391	95.24	-12.3149	19.9977	-0.0164329	1.84882	293.15	293.15	0	368.419	368.419	0.0837692	0.0837907

392	95.41	-12.2629	20.0008	-0.0163627	1.85549	293.15	293.15	0	368.588	368.588	0.0838071	0.0838293

393	95.57	-12.1535	20.0008	-0.0162159	1.86011	293.15	293.15	0	368.763	368.763	0.083845	0.0838676

394	95.74	-12.0916	20.0008	-0.0161326	1.86265	293.15	293.15	0	368.93	368.93	0.0838845	0.0839065

395	95.91	-12.1275	20.0008	-0.0161796	1.87247	293.15	293.15	0	369.099	369.099	0.083922	0.0839443

396	96.07	-12.2093	19.9935	-0.016288	1.87692	293.15	293.15	0	369.273	369.273	0.0839603	0.0839832

397	96.24	-12.1698	19.9966	-0.0162345	1.88003	293.15	293.15	0	369.42	369.42	0.0839988	0.0840218

398	96.4	-12.1329	20.0008	-0.0161844	1.88509	293.15	293.15	0	369.586	369.586	0.0840364	0.0840594

399	96.58	-12.1866	19.9946	-0.0162551	1.89119	293.15	293.15	0	369.757	369.757	0.0840752	0.0840994

400	96.74	-12.2124	19.9966	-0.0162889	1.89821	293.15	293.15	0	369.93	369.93	0.0841135	0.0841371

401	96.91	-12.2149	20.0008	-0.0162914	1.90094	293.15	293.15	0	370.094	370.094	0.084153	0.0841768

402	97.08	-12.1843	20.0008	-0.0162497	1.90628	293.15	293.15	0	370.261	370.261	0.0841921	0.0842148

403	97.24	-12.1594	19.9946	-0.0162157	1.91541	293.15	293.15	0	370.441	370.441	0.0842295	0.0842529

404	97.42	-12.1488	19.9966	-0.0162008	1.91831	293.15	293.15	0	370.598	370.598	0.0842683	0.0842927

405	97.58	-12.1756	20.0008	-0.0162357	1.92212	293.15	293.15	0	370.762	370.762	0.084307	0.0843309

406	97.75	-12.1872	20.0008	-0.0162503	1.92636	293.15	293.15	0	370.935	370.935	0.0843445	0.0843687

407	97.91	-12.1669	20.0008	-0.0162225	1.93579	293.15	293.15	0	371.099	371.099	0.0843827	0.0844068

408	98.08	-12.0445	20.0008	-0.0160585	1.93839	293.15	293.15	0	371.272	371.272	0.0844211	0.0844454

409	98.25	-11.9376	20.0008	-0.0159151	1.94258	293.15	293.15	0	371.429	371.429	0.0844598	0.084484

410	98.41	-11.9479	20.0008	-0.015928	1.94818	293.15	293.15	0	371.593	371.593	0.0844976	0.0845223

411	98.58	-11.9999	20.0008	-0.0159965	1.95539	293.15	293.15	0	371.766	371.766	0.084536	0.084561

412	98.75	-12.0004	20.0008	-0.0159965	1.95987	293.15	293.15	0	371.938	371.938	0.0845745	0.0845994

413	98.91	-12.0494	20.0008	-0.0160609	1.9628	293.15	293.15	0	372.087	372.087	0.084613	0.0846382

414	99.08	-12.0739	20.0008	-0.0160929	1.96809	293.15	293.15	0	372.26	372.26	0.0846519	0.0846768

415	99.25	-12.0268	20.0008	-0.0160293	1.97241	293.15	293.15	0	372.425	372.425	0.0846903	0.0847152

416	99.42	-11.9136	20.0008	-0.0158775	1.98022	293.15	293.15	0	372.594	372.594	0.0847283	0.084754

417	99.58	-11.8035	20.0008	-0.01573	1.98532	293.15	293.15	0	372.762	372.762	0.0847667	0.0847924

418	99.75	-11.7614	19.9987	-0.0156731	1.99089	293.15	293.15	0	372.931	372.931	0.0848054	0.0848311

419	99.92	-11.7891	19.9977	-0.0157093	1.99272	293.15	293.15	0	373.084	373.084	0.0848436	0.0848695

420	100.08	-11.7887	20.0008	-0.015708	1.92273	293.15	293.15	0	373.072	373.072	0.0848819	0.0849073

421	100.22	-11.7822	19.9935	-0.0156986	1.79526	293.15	293.15	0	372.907	372.907	0.0849129	0.0849384

422	100.28	-11.4448	19.9977	-0.0152489	1.68418	293.15	293.15	0	372.741	372.741	0.0849282	0.0849517

423	100.25	-10.0892	20.0008	-0.0134428	1.58975	293.15	293.15	0	372.57	372.57	0.0849273	0.0849465

424	100.17	-7.79839	20.0008	-0.0103908	1.51362	293.15	293.15	0	372.405	372.405	0.0849135	0.0849275

425	100.05	-5.02367	20.0008	-0.00669391	1.45539	293.15	293.15	0	372.248	372.248	0.0848902	0.0848988

426	99.88	-1.94977	20.0008	-0.00259815	1.4052	293.15	293.15	0	372.077	372.077	0.084857	0.0848603

427	99.7	1.09215	20.0008	0.00145542	1.36171	293.15	293.15	0	371.903	371.903	0.0848184	0.0848183

428	99.49	4.03757	20.0008	0.00538085	1.33131	293.15	293.15	0	371.738	371.738	0.0847748	0.0847704

429	99.26	6.81391	19.9946	0.00908149	1.31188	293.15	293.15	0	371.567	371.567	0.0847253	0.0847181

430	99.03	9.23675	19.9966	0.0123115	1.29776	293.15	293.15	0	371.401	371.401	0.0846751	0.0846651

431	98.8	11.3364	20.0008	0.0151112	1.28526	293.15	293.15	0	371.245	371.245	0.0846225	0.084611

432	98.56	12.9379	20.0008	0.0172471	1.2797	293.15	293.15	0	371.072	371.072	0.0845692	0.0845559

433	98.33	14.1524	20.0008	0.0188674	1.27688	293.15	293.15	0	370.909	370.909	0.0845176	0.0845034

434	98.1	15.0678	19.9956	0.0200891	1.27796	293.15	293.15	0	370.735	370.735	0.0844644	0.0844498

435	97.86	15.8059	20.0008	0.0210748	1.27624	293.15	293.15	0	370.571	370.571	0.084412	0.0843959

436	97.64	16.3152	20.0008	0.0217552	1.27689	293.15	293.15	0	370.405	370.405	0.084361	0.0843452

437	97.43	16.5743	20.0008	0.0221021	1.28058	293.15	293.15	0	370.243	370.243	0.0843116	0.0842959

438	97.22	16.6825	20.0008	0.0222478	1.28252	293.15	293.15	0	370.078	370.078	0.0842634	0.0842476

439	97.01	16.7225	19.9966	0.0223025	1.28129	293.15	293.15	0	369.913	369.913	0.0842155	0.0842001

440	96.81	16.6057	19.9946	0.0221481	1.28147	293.15	293.15	0	369.74	369.74	0.0841688	0.0841536

441	96.61	16.4159	19.9914	0.0218963	1.28737	293.15	293.15	0	369.569	369.569	0.084123	0.0841079

442	96.42	16.1541	19.9935	0.0215482	1.29083	293.15	293.15	0	369.412	369.412	0.0840774	0.0840629

443	96.23	15.8332	19.9977	0.0211214	1.29053	293.15	293.15	0	369.246	369.246	0.0840338	0.0840196

444	96.05	15.5194	19.9987	0.0207041	1.28805	293.15	293.15	0	369.076	369.076	0.0839909	0.0839768

445	95.86	15.2516	19.9977	0.0203478	1.28798	293.15	293.15	0	368.908	368.908	0.0839488	0.083935

446	95.69	14.9373	19.9904	0.0199296	1.28617	293.15	293.15	0	368.735	368.735	0.0839074	0.0838938

447	95.51	14.5522	19.9987	0.0194168	1.28369	293.15	293.15	0	368.566	368.566	0.0838665	0.0838534

448	95.34	14.2052	20.0008	0.0189548	1.28226	293.15	293.15	0	368.407	368.407	0.0838264	0.0838133

449	95.16	13.9717	20.0008	0.0186442	1.27986	293.15	293.15	0	368.241	368.241	0.0837859	0.0837731

450	95	13.8071	20.0008	0.0184254	1.27774	293.15	293.15	0	368.074	368.074	0.0837474	0.0837343

451	94.82	13.6645	20.0008	0.0182362	1.27257	293.15	293.15	0	367.905	367.905	0.0837074	0.0836937

452	94.65	13.5444	20.0008	0.0180768	1.26933	293.15	293.15	0	367.739	367.739	0.0836686	0.0836551

453	94.49	13.4721	20.0008	0.0179812	1.2666	293.15	293.15	0	367.567	367.567	0.0836307	0.0836173

454	94.32	13.4323	20.0008	0.0179289	1.26401	293.15	293.15	0	367.409	367.409	0.0835912	0.0835781

455	94.15	13.3685	20.0008	0.0178447	1.25997	293.15	293.15	0	367.247	367.247	0.0835527	0.0835396

456	93.98	13.2863	20.0008	0.0177358	1.25395	293.15	293.15	0	367.073	367.073	0.0835138	0.0835007

457	93.82	13.1528	20.0008	0.0175584	1.24895	293.15	293.15	0	366.909	366.909	0.0834762	0.0834631

458	93.65	13.0381	20.0008	0.0174062	1.24658	293.15	293.15	0	366.743	366.743	0.0834373	0.0834246

459	93.49	12.9833	20.0008	0.0173339	1.23833	293.15	293.15	0	366.571	366.571	0.0833997	0.0833866

460	93.32	12.889	20.0008	0.0172088	1.23221	293.15	293.15	0	366.406	366.406	0.0833614	0.0833481

461	93.16	12.8356	20.0008	0.0171384	1.22837	293.15	293.15	0	366.232	366.232	0.0833234	0.08331

462	92.99	12.7333	20.0008	0.0170026	1.22593	293.15	293.15	0	366.078	366.078	0.083285	0.083272

463	92.83	12.6209	20.0008	0.0168534	1.22048	293.15	293.15	0	365.912	365.912	0.0832476	0.0832345

464	92.66	12.6034	20.0008	0.016831	1.21447	293.15	293.15	0	365.741	365.741	0.0832083	0.0831944

465	92.49	12.6303	19.9966	0.0168677	1.2115	293.15	293.15	0	365.575	365.575	0.0831695	0.0831553

466	92.32	12.6124	19.9998	0.0168446	1.20573	293.15	293.15	0	365.403	365.403	0.0831317	0.0831172

467	92.16	12.6111	19.9925	0.0168438	1.2014	293.15	293.15	0	365.245	365.245	0.0830934	0.0830787

468	91.99	12.7047	19.9935	0.0169696	1.19542	293.15	293.15	0	365.08	365.08	0.0830553	0.0830401

469	91.82	12.7808	20.0008	0.0170721	1.1906	293.15	293.15	0	364.907	364.907	0.0830161	0.0830006

470	91.65	12.8524	19.9925	0.0171686	1.1871	293.15	293.15	0	364.738	364.738	0.0829769	0.082962

471	91.49	12.9136	19.9935	0.0172512	1.17874	293.15	293.15	0	364.568	364.568	0.0829402	0.0829241

472	91.32	12.9131	20.0008	0.0172514	1.17241	293.15	293.15	0	364.404	364.404	0.0829015	0.0828859

473	91.15	12.8552	19.9935	0.0171749	1.17022	293.15	293.15	0	364.246	364.246	0.0828624	0.082847

474	90.98	12.7875	19.9977	0.0170854	1.16923	293.15	293.15	0	364.076	364.076	0.0828227	0.082807

475	90.81	12.7702	19.9935	0.0170632	1.16266	293.15	293.15	0	363.903	363.903	0.0827851	0.0827686

476	90.65	12.8175	19.9904	0.0171272	1.15593	293.15	293.15	0	363.734	363.734	0.0827467	0.0827302

477	90.48	12.8207	19.9966	0.0171323	1.15253	293.15	293.15	0	363.581	363.581	0.0827078	0.0826912

478	90.31	12.8051	20.0008	0.0171123	1.14667	293.15	293.15	0	363.409	363.409	0.0826704	0.082653

479	90.15	12.8291	20.0008	0.0171452	1.14308	293.15	293.15	0	363.245	363.245	0.0826316	0.0826146

480	89.98	12.8767	20.0008	0.0172097	1.13808	293.15	293.15	0	363.079	363.079	0.0825928	0.0825762

481	89.81	12.8907	20.0008	0.0172293	1.13112	293.15	293.15	0	362.899	362.899	0.0825544	0.0825369

482	89.64	12.8788	19.9946	0.0172142	1.13006	293.15	293.15	0	362.741	362.741	0.0825147	0.082498

483	89.48	12.7832	19.9956	0.0170872	1.12348	293.15	293.15	0	362.585	362.585	0.0824771	0.0824606

484	89.31	12.766	20.0008	0.0170652	1.11794	293.15	293.15	0	362.405	362.405	0.0824381	0.0824208

485	89.14	12.8009	20.0008	0.0171128	1.11336	293.15	293.15	0	362.24	362.24	0.0823999	0.082382

486	88.97	12.8613	20.0008	0.0171943	1.10925	293.15	293.15	0	362.067	362.067	0.0823616	0.0823427

487	88.8	12.9527	19.9956	0.0173175	1.10573	293.15	293.15	0	361.904	361.904	0.0823214	0.0823033

488	88.64	12.9876	19.9904	0.0173649	1.10192	293.15	293.15	0	361.739	361.739	0.082283	0.0822646

489	88.47	12.9755	19.9946	0.0173497	1.09876	293.15	293.15	0	361.573	361.573	0.082244	0.0822259

490	88.3	12.9598	20.0008	0.0173295	1.09213	293.15	293.15	0	361.409	361.409	0.0822062	0.0821876

491	88.13	12.9293	20.0008	0.0172896	1.09178	293.15	293.15	0	361.237	361.237	0.0821674	0.0821488

492	87.97	12.9149	19.9966	0.0172712	1.08304	293.15	293.15	0	361.072	361.072	0.0821293	0.0821099

493	87.8	12.8735	19.9935	0.0172166	1.07916	293.15	293.15	0	360.915	360.915	0.0820914	0.0820724

494	87.64	12.8795	20.0008	0.0172256	1.07474	293.15	293.15	0	360.746	360.746	0.082052	0.0820332

495	87.47	12.8573	20.0008	0.0171968	1.07158	293.15	293.15	0	360.578	360.578	0.0820134	0.0819943

496	87.3	12.8768	19.9977	0.0172237	1.06518	293.15	293.15	0	360.405	360.405	0.0819746	0.0819549

497	87.13	12.8725	19.9987	0.0172188	1.05936	293.15	293.15	0	360.24	360.24	0.0819361	0.0819163

498	86.96	12.8405	20.0008	0.0171769	1.05602	293.15	293.15	0	360.079	360.079	0.0818974	0.0818774

499	86.8	12.8332	20.0008	0.017168	1.05313	293.15	293.15	0	359.91	359.91	0.0818585	0.0818387

500	86.63	12.7838	20.0008	0.0171028	1.04492	293.15	293.15	0	359.743	359.743	0.0818202	0.0817997

501	86.46	12.7502	20.0008	0.0170588	1.04336	293.15	293.15	0	359.574	359.574	0.081781	0.0817603

502	86.29	12.6626	20.0008	0.0169423	1.04028	293.15	293.15	0	359.401	359.401	0.0817423	0.0817224

503	86.13	12.5533	20.0008	0.0167969	1.0343	293.15	293.15	0	359.236	359.236	0.0817045	0.0816841

504	85.96	12.5301	20.0008	0.0167667	1.0283	293.15	293.15	0	359.078	359.078	0.0816661	0.0816453

505	85.79	12.5148	20.0008	0.016747	1.02276	293.15	293.15	0	358.906	358.906	0.0816279	0.0816069

506	85.63	12.5009	20.0008	0.0167293	1.01939	293.15	293.15	0	358.742	358.742	0.0815893	0.0815684

507	85.46	12.5244	19.9946	0.0167617	1.01439	293.15	293.15	0	358.576	358.576	0.0815503	0.0815292

508	85.29	12.5948	19.9966	0.0168567	1.00671	293.15	293.15	0	358.396	358.396	0.0815118	0.0814905

509	85.13	12.562	19.9956	0.0168136	1.00372	293.15	293.15	0	358.248	358.248	0.0814732	0.0814522

510	84.96	12.5585	20.0008	0.0168098	0.999963	293.15	293.15	0	358.084	358.084	0.0814346	0.0814135

511	84.78	12.6092	19.9956	0.0168785	0.998056	293.15	293.15	0	357.91	357.91	0.0813952	0.081373

512	84.61	12.6313	19.9904	0.016909	0.991649	293.15	293.15	0	357.738	357.738	0.081356	0.0813333

513	84.45	12.656	20.0008	0.0169429	0.989263	293.15	293.15	0	357.573	357.573	0.0813171	0.0812951

514	84.28	12.6132	20.0008	0.0168864	0.985128	293.15	293.15	0	357.4	357.4	0.0812786	0.0812567

515	84.12	12.5619	20.0008	0.0168185	0.982438	293.15	293.15	0	357.244	357.244	0.0812404	0.0812187

516	83.95	12.5337	19.9914	0.0167816	0.976303	293.15	293.15	0	357.071	357.071	0.0812018	0.0811802

517	83.79	12.5289	19.9946	0.0167761	0.97003	293.15	293.15	0	356.899	356.899	0.0811638	0.0811413

518	83.62	12.4893	20.0008	0.0167239	0.966488	293.15	293.15	0	356.743	356.743	0.0811262	0.0811031

519	83.45	12.4933	20.0008	0.0167301	0.964481	293.15	293.15	0	356.586	356.586	0.0810868	0.0810634

520	83.28	12.5201	20.0008	0.0167668	0.955827	293.15	293.15	0	356.407	356.407	0.0810473	0.0810245

521	83.11	12.5574	20.0008	0.0168176	0.9527	293.15	293.15	0	356.239	356.239	0.0810085	0.0809849

522	82.95	12.5922	19.9925	0.0168651	0.946706	293.15	293.15	0	356.066	356.066	0.0809703	0.0809465

523	82.78	12.5189	19.9977	0.0167678	0.945091	293.15	293.15	0	355.918	355.918	0.0809312	0.0809074

524	82.6	12.477	20.0008	0.0167125	0.942184	293.15	293.15	0	355.75	355.75	0.0808912	0.0808673

525	82.44	12.4817	20.0008	0.0167196	0.936799	293.15	293.15	0	355.582	355.582	0.0808531	0.0808294

526	82.27	12.3972	20.0008	0.0166073	0.932781	293.15	293.15	0	355.404	355.404	0.0808143	0.0807908

527	82.11	12.353	19.9946	0.0165489	0.926941	293.15	293.15	0	355.242	355.242	0.0807765	0.0807527

528	81.95	12.3541	19.9966	0.0165511	0.921863	293.15	293.15	0	355.076	355.076	0.0807392	0.0807147

529	81.78	12.3729	20.0008	0.0165773	0.917009	293.15	293.15	0	354.905	354.905	0.0806991	0.0806751

530	81.6	12.3579	20.0008	0.016558	0.912611	293.15	293.15	0	354.732	354.732	0.0806603	0.0806355

531	81.44	12.3886	19.9946	0.0165999	0.908768	293.15	293.15	0	354.568	354.568	0.0806218	0.0805965

532	81.27	12.4288	19.9956	0.0166547	0.90868	293.15	293.15	0	354.42	354.42	0.0805824	0.0805575

533	81.11	12.4418	20.0008	0.0166729	0.898238	293.15	293.15	0	354.247	354.247	0.0805447	0.0805198

534	80.94	12.4036	20.0008	0.0166226	0.896758	293.15	293.15	0	354.074	354.074	0.080506	0.0804807

535	80.77	12.4056	20.0008	0.016626	0.892547	293.15	293.15	0	353.91	353.91	0.0804675	0.0804422

536	80.6	12.409	20.0008	0.0166315	0.885965	293.15	293.15	0	353.737	353.737	0.0804277	0.080403

537	80.44	12.3315	20.0008	0.0165284	0.881887	293.15	293.15	0	353.563	353.563	0.0803896	0.0803643

538	80.27	12.2027	20.0008	0.0163566	0.879157	293.15	293.15	0	353.416	353.416	0.0803511	0.0803252

539	80.1	12.11	20.0008	0.0162331	0.877001	293.15	293.15	0	353.242	353.242	0.080312	0.0802869

540	79.94	12.1138	20.0008	0.0162391	0.874068	293.15	293.15	0	353.071	353.071	0.0802733	0.0802482

541	79.77	12.1556	20.0008	0.0162959	0.866524	293.15	293.15	0	352.906	352.906	0.0802346	0.0802094

542	79.6	12.1858	19.9914	0.0163372	0.864192	293.15	293.15	0	352.732	352.732	0.0801952	0.0801702

543	79.43	12.2378	19.9946	0.0164078	0.859444	293.15	293.15	0	352.568	352.568	0.0801577	0.0801309

544	79.27	12.2933	20.0008	0.016483	0.854821	293.15	293.15	0	352.405	352.405	0.0801188	0.0800925

545	79.1	12.2608	20.0008	0.0164402	0.848115	293.15	293.15	0	352.247	352.247	0.0800802	0.0800541

546	78.93	12.1743	20.0008	0.0163251	0.845565	293.15	293.15	0	352.074	352.074	0.0800412	0.0800149

547	78.76	12.1417	20.0008	0.0162822	0.841319	293.15	293.15	0	351.905	351.905	0.080002	0.0799756

548	78.6	12.19	20.0008	0.0163479	0.838282	293.15	293.15	0	351.737	351.737	0.0799628	0.0799371

549	78.43	12.2114	20.0008	0.0163774	0.831682	293.15	293.15	0	351.564	351.564	0.0799242	0.0798978

550	78.26	12.1943	19.9925	0.0163552	0.827057	293.15	293.15	0	351.404	351.404	0.0798859	0.0798591

551	78.1	12.2546	19.9977	0.016437	0.823032	293.15	293.15	0	351.243	351.243	0.0798483	0.0798211

552	77.93	12.3003	20.0008	0.0164991	0.819866	293.15	293.15	0	351.079	351.079	0.0798086	0.0797814

553	77.76	12.2946	20.0008	0.0164923	0.814237	293.15	293.15	0	350.906	350.906	0.0797698	0.0797426

554	77.59	12.32	20.0008	0.0165272	0.811897	293.15	293.15	0	350.738	350.738	0.0797306	0.0797029

555	77.42	12.3587	19.9935	0.0165799	0.808218	293.15	293.15	0	350.568	350.568	0.0796924	0.0796648

556	77.26	12.3503	19.9977	0.0165695	0.803755	293.15	293.15	0	350.402	350.402	0.079654	0.0796257

557	77.09	12.3555	20.0008	0.0165773	0.79909	293.15	293.15	0	350.246	350.246	0.0796141	0.0795866

558	76.92	12.3837	20.0008	0.016616	0.794257	293.15	293.15	0	350.075	350.075	0.0795757	0.079548

559	76.75	12.3601	20.0008	0.0165851	0.792046	293.15	293.15	0	349.91	349.91	0.0795364	0.0795087

560	76.59	12.3073	20.0008	0.016515	0.78469	293.15	293.15	0	349.735	349.735	0.0794982	0.0794702

561	76.42	12.2249	20.0008	0.0164054	0.779491	293.15	293.15	0	349.58	349.58	0.0794596	0.0794308

562	76.25	12.1404	19.9956	0.0162927	0.776851	293.15	293.15	0	349.408	349.408	0.0794206	0.079392

563	76.09	12.1084	20.0008	0.0162507	0.772259	293.15	293.15	0	349.243	349.243	0.079383	0.0793537

564	75.92	12.1042	20.0008	0.0162459	0.766237	293.15	293.15	0	349.078	349.078	0.0793434	0.0793146

565	75.75	12.0947	20.0008	0.016234	0.76433	293.15	293.15	0	348.906	348.906	0.0793044	0.0792757

566	75.58	12.0642	20.0008	0.0161938	0.760913	293.15	293.15	0	348.732	348.732	0.0792654	0.0792365

567	75.41	12.0776	20.0008	0.0162125	0.758582	293.15	293.15	0	348.569	348.569	0.0792266	0.0791975

568	75.25	12.1268	20.0008	0.0162795	0.7562	293.15	293.15	0	348.402	348.402	0.0791877	0.0791581

569	75.08	12.1918	20.0008	0.0163676	0.749841	293.15	293.15	0	348.248	348.248	0.0791484	0.0791189

570	74.91	12.2103	20.0008	0.0163933	0.746489	293.15	293.15	0	348.076	348.076	0.07911	0.0790799

571	74.74	12.1996	20.0008	0.0163797	0.741954	293.15	293.15	0	347.91	347.91	0.0790719	0.0790409

572	74.58	12.1442	20.0008	0.0163061	0.737279	293.15	293.15	0	347.737	347.737	0.0790321	0.0790021

573	74.41	12.0923	20.0008	0.0162372	0.733409	293.15	293.15	0	347.566	347.566	0.0789944	0.0789636

574	74.24	12.0296	20.0008	0.0161539	0.730914	293.15	293.15	0	347.409	347.409	0.078955	0.0789241

575	74.07	11.9638	20.0008	0.0160663	0.725538	293.15	293.15	0	347.243	347.243	0.0789166	0.0788854

576	73.91	11.9607	19.9977	0.016063	0.718056	293.15	293.15	0	347.074	347.074	0.0788784	0.0788464

577	73.74	12.0128	19.9904	0.0161337	0.714291	293.15	293.15	0	346.906	346.906	0.0788394	0.0788076

578	73.57	12.0734	19.9987	0.0162161	0.710978	293.15	293.15	0	346.733	346.733	0.0787996	0.0787675

579	73.4	12.1288	19.9987	0.0162913	0.708265	293.15	293.15	0	346.585	346.585	0.0787605	0.0787284

580	73.23	12.205	19.9977	0.0163944	0.702806	293.15	293.15	0	346.418	346.418	0.078722	0.0786896

581	73.07	12.2096	19.9935	0.0164014	0.699484	293.15	293.15	0	346.248	346.248	0.0786827	0.0786507

582	72.9	12.1432	19.9977	0.0163131	0.698077	293.15	293.15	0	346.08	346.08	0.0786438	0.0786113

583	72.73	12.0628	20.0008	0.0162059	0.692048	293.15	293.15	0	345.909	345.909	0.078606	0.0785731

584	72.57	12.0143	19.9946	0.0161415	0.686469	293.15	293.15	0	345.743	345.743	0.0785669	0.0785342

585	72.4	12.0102	19.9966	0.0161368	0.68238	293.15	293.15	0	345.571	345.571	0.0785283	0.0784961

586	72.23	12.0067	20.0008	0.0161329	0.678914	293.15	293.15	0	345.406	345.406	0.0784891	0.078456

587	72.06	12.0129	20.0008	0.0161421	0.677206	293.15	293.15	0	345.251	345.251	0.078449	0.0784168

588	71.9	12.0295	19.9904	0.0161651	0.671846	293.15	293.15	0	345.077	345.077	0.0784116	0.0783782

589	71.73	12.0405	19.9956	0.0161808	0.667625	293.15	293.15	0	344.904	344.904	0.0783724	0.0783388

590	71.56	12.0293	19.9956	0.0161666	0.661002	293.15	293.15	0	344.741	344.741	0.0783351	0.0783011

591	71.4	12.0251	20.0008	0.0161618	0.659739	293.15	293.15	0	344.567	344.567	0.0782953	0.078262

592	71.22	12.0438	20.0008	0.0161877	0.655882	293.15	293.15	0	344.403	344.403	0.0782557	0.0782218

593	71.06	12.0952	20.0008	0.0162576	0.651459	293.15	293.15	0	344.247	344.247	0.0782173	0.0781834

594	70.89	12.0764	20.0008	0.0162332	0.648489	293.15	293.15	0	344.073	344.073	0.0781784	0.0781439

595	70.72	12.0507	20.0008	0.0161995	0.64526	293.15	293.15	0	343.909	343.909	0.0781395	0.0781046

596	70.55	12.0241	20.0008	0.0161644	0.642063	293.15	293.15	0	343.737	343.737	0.0781009	0.0780658

597	70.39	12.0135	20.0008	0.0161511	0.63642	293.15	293.15	0	343.572	343.572	0.0780614	0.0780272

598	70.22	11.9805	20.0008	0.0161074	0.633036	293.15	293.15	0	343.406	343.406	0.0780228	0.077988

599	70.05	11.9977	20.0008	0.0161314	0.62917	293.15	293.15	0	343.246	343.246	0.0779837	0.0779487

600	69.89	12.0429	20.0008	0.0161929	0.625951	293.15	293.15	0	343.078	343.078	0.0779452	0.0779102

601	69.72	12.109	20.0008	0.0162827	0.619304	293.15	293.15	0	342.905	342.905	0.0779068	0.0778712

602	69.55	12.1757	19.9925	0.0163733	0.61629	293.15	293.15	0	342.735	342.735	0.0778668	0.0778315

603	69.39	12.1752	19.9987	0.0163733	0.611335	293.15	293.15	0	342.567	342.567	0.0778288	0.0777936

604	69.22	12.0722	20.0008	0.0162357	0.609715	293.15	293.15	0	342.401	342.401	0.0777893	0.0777545

605	69.05	11.9637	20.0008	0.0160905	0.603007	293.15	293.15	0	342.246	342.246	0.0777502	0.0777158

606	68.89	11.8962	20.0008	0.0160006	0.599871	293.15	293.15	0	342.079	342.079	0.0777116	0.077677

607	68.71	11.8337	20.0008	0.0159174	0.598317	293.15	293.15	0	341.91	341.91	0.0776718	0.0776368

608	68.55	11.7535	20.0008	0.0158103	0.594298	293.15	293.15	0	341.736	341.736	0.0776334	0.0775984

609	68.38	11.7205	20.0008	0.0157666	0.587816	293.15	293.15	0	341.569	341.569	0.0775953	0.0775593

610	68.22	11.7102	19.9998	0.0157536	0.586536	293.15	293.15	0	341.408	341.408	0.0775561	0.0775205

611	68.05	11.7026	19.9904	0.0157441	0.581648	293.15	293.15	0	341.242	341.242	0.0775171	0.0774815

612	67.88	11.7034	19.9956	0.015746	0.576797	293.15	293.15	0	341.078	341.078	0.0774785	0.0774429

613	67.71	11.7095	19.9904	0.0157551	0.575164	293.15	293.15	0	340.912	340.912	0.077439	0.0774034

614	67.54	11.7171	19.9966	0.0157661	0.570871	293.15	293.15	0	340.732	340.732	0.0773991	0.0773633

615	67.38	11.6806	19.9956	0.0157177	0.564751	293.15	293.15	0	340.568	340.568	0.0773616	0.0773253

616	67.21	11.6755	20.0008	0.0157117	0.560862	293.15	293.15	0	340.41	340.41	0.0773232	0.0772862

617	67.04	11.6746	19.9956	0.0157113	0.555344	293.15	293.15	0	340.247	340.247	0.0772837	0.0772467

618	66.88	11.6642	19.9956	0.0156981	0.552669	293.15	293.15	0	340.072	340.072	0.0772447	0.0772077

619	66.71	11.7075	20.0008	0.0157572	0.553026	293.15	293.15	0	339.909	339.909	0.0772055	0.0771681

620	66.54	11.7462	20.0008	0.0158101	0.544188	293.15	293.15	0	339.737	339.737	0.0771667	0.0771295

621	66.38	11.7757	20.0008	0.0158505	0.541105	293.15	293.15	0	339.572	339.572	0.077128	0.0770911

622	66.21	11.7307	20.0112	0.0157907	0.539111	293.15	293.15	0	339.399	339.399	0.0770887	0.0770519

623	66.04	11.6654	20.0071	0.0157036	0.535316	293.15	293.15	0	339.252	339.252	0.0770507	0.0770128

624	65.87	11.6571	20.0008	0.0156932	0.53379	293.15	293.15	0	339.078	339.078	0.0770111	0.0769735

625	65.71	11.6137	20.0008	0.0156357	0.526358	293.15	293.15	0	338.906	338.906	0.0769726	0.0769351

626	65.54	11.5672	20.0008	0.0155738	0.523777	293.15	293.15	0	338.741	338.741	0.0769338	0.0768966

627	65.37	11.5223	19.9914	0.0155141	0.51875	293.15	293.15	0	338.578	338.578	0.0768955	0.0768569

628	65.21	11.5753	19.9904	0.0155863	0.515299	293.15	293.15	0	338.404	338.404	0.0768557	0.0768176

629	65.04	11.6306	19.9904	0.0156615	0.513299	293.15	293.15	0	338.232	338.232	0.0768164	0.0767779

630	64.87	11.6022	19.9998	0.0156242	0.510893	293.15	293.15	0	338.075	338.075	0.0767771	0.0767385

631	64.7	11.5083	20.0008	0.0154984	0.506843	293.15	293.15	0	337.91	337.91	0.0767381	0.0766991

632	64.53	11.4116	20.0008	0.015369	0.502867	293.15	293.15	0	337.74	337.74	0.0766986	0.0766604

633	64.36	11.3651	20.0008	0.0153072	0.497505	293.15	293.15	0	337.573	337.573	0.07666	0.0766213

634	64.2	11.3834	20.0008	0.0153326	0.493437	293.15	293.15	0	337.4	337.4	0.0766209	0.0765817

635	64.03	11.4199	20.0008	0.0153825	0.489594	293.15	293.15	0	337.252	337.252	0.0765826	0.0765433

636	63.87	11.4537	20.0008	0.0154289	0.484521	293.15	293.15	0	337.084	337.084	0.0765443	0.0765047

637	63.7	11.4569	20.0008	0.015434	0.481523	293.15	293.15	0	336.915	336.915	0.0765045	0.0764651

638	63.53	11.4135	20.0008	0.0153763	0.480283	293.15	293.15	0	336.741	336.741	0.0764648	0.0764257

639	63.36	11.3649	20.0008	0.0153116	0.478332	293.15	293.15	0	336.574	336.574	0.0764254	0.0763855

640	63.19	11.3455	20.0008	0.0152861	0.472571	293.15	293.15	0	336.404	336.404	0.0763868	0.0763474

641	63.02	11.3407	20.0008	0.0152805	0.469322	293.15	293.15	0	336.247	336.247	0.0763479	0.0763078

642	62.86	11.4052	20.0008	0.0153681	0.465121	293.15	293.15	0	336.082	336.082	0.0763096	0.0762689

643	62.69	11.4823	20.0008	0.0154729	0.460419	293.15	293.15	0	335.91	335.91	0.076271	0.0762306

644	62.53	11.5485	20.0008	0.0155628	0.455916	293.15	293.15	0	335.746	335.746	0.0762321	0.0761914

645	62.36	11.5324	20.0008	0.0155419	0.452478	293.15	293.15	0	335.573	335.573	0.0761925	0.0761519

646	62.19	11.5036	20.0008	0.0155039	0.449295	293.15	293.15	0	335.407	335.407	0.0761538	0.076113

647	62.02	11.4728	20.0008	0.0154632	0.444161	293.15	293.15	0	335.252	335.252	0.0761141	0.0760739

648	61.86	11.4088	20.0008	0.0153777	0.438085	293.15	293.15	0	335.078	335.078	0.0760759	0.0760358

649	61.69	11.3053	19.9966	0.0152389	0.437209	293.15	293.15	0	334.906	334.906	0.0760365	0.0759962

650	61.53	11.234	19.9998	0.0151435	0.434066	293.15	293.15	0	334.749	334.749	0.0759981	0.0759573

651	61.35	11.2312	20.0008	0.0151406	0.431733	293.15	293.15	0	334.576	334.576	0.075959	0.0759174

652	61.19	11.2649	19.9914	0.0151868	0.426155	293.15	293.15	0	334.403	334.403	0.0759198	0.0758778

653	61.02	11.3277	19.9904	0.0152722	0.421194	293.15	293.15	0	334.24	334.24	0.0758813	0.07584

654	60.85	11.424	19.9935	0.0154029	0.418855	293.15	293.15	0	334.073	334.073	0.0758415	0.0757995

655	60.68	11.5011	20.0008	0.0155075	0.416456	293.15	293.15	0	333.9	333.9	0.0758021	0.0757604

656	60.51	11.4243	20.0008	0.0154048	0.412934	293.15	293.15	0	333.739	333.739	0.075763	0.0757209

657	60.35	11.3232	19.9987	0.0152692	0.409682	293.15	293.15	0	333.579	333.579	0.0757236	0.0756816

658	60.18	11.275	19.9977	0.0152051	0.405167	293.15	293.15	0	333.406	333.406	0.075685	0.075643

659	60.02	11.2482	20.0008	0.0151697	0.402559	293.15	293.15	0	333.241	333.241	0.0756457	0.0756043

660	59.85	11.23	20.0008	0.0151458	0.40051	293.15	293.15	0	333.074	333.074	0.0756068	0.0755652

661	59.68	11.1193	20.0008	0.0149973	0.394051	293.15	293.15	0	332.905	332.905	0.0755682	0.0755258

662	59.51	11.0622	20.0008	0.0149211	0.391603	293.15	293.15	0	332.731	332.731	0.075529	0.0754867

663	59.35	11.081	19.9998	0.0149472	0.38837	293.15	293.15	0	332.583	332.583	0.0754907	0.075448

664	59.18	11.1221	19.9904	0.0150034	0.384544	293.15	293.15	0	332.417	332.417	0.075452	0.0754089

665	59.01	11.1581	19.9966	0.0150528	0.380536	293.15	293.15	0	332.246	332.246	0.0754133	0.0753698

666	58.85	11.1563	20.0008	0.015051	0.375843	293.15	293.15	0	332.073	332.073	0.0753733	0.0753307

667	58.68	11.1308	20.0008	0.0150174	0.372391	293.15	293.15	0	331.907	331.907	0.0753342	0.0752912

668	58.51	11.1045	19.9998	0.0149827	0.369716	293.15	293.15	0	331.736	331.736	0.0752948	0.0752517

669	58.34	11.0716	19.9904	0.0149391	0.364806	293.15	293.15	0	331.578	331.578	0.0752557	0.0752122

670	58.18	11.0036	19.9904	0.0148481	0.363128	293.15	293.15	0	331.415	331.415	0.0752161	0.0751735

671	58.01	10.9691	19.9904	0.0148023	0.359164	293.15	293.15	0	331.241	331.241	0.0751775	0.0751337

672	57.84	11.0047	19.9904	0.014851	0.35691	293.15	293.15	0	331.068	331.068	0.0751381	0.0750953

673	57.67	11.0354	19.9956	0.0148932	0.350271	293.15	293.15	0	330.904	330.904	0.0750994	0.0750559

674	57.51	11.0342	20.0008	0.0148924	0.34806	293.15	293.15	0	330.731	330.731	0.0750601	0.0750168

675	57.34	11.0824	20.0008	0.0149582	0.345059	293.15	293.15	0	330.583	330.583	0.0750218	0.0749776

676	57.17	11.0894	20.0008	0.0149684	0.34308	293.15	293.15	0	330.412	330.412	0.0749825	0.0749384

677	57	11.0247	20.0008	0.0148818	0.339444	293.15	293.15	0	330.246	330.246	0.0749429	0.0748987

678	56.84	11.0244	19.9914	0.0148821	0.334848	293.15	293.15	0	330.073	330.073	0.0749049	0.0748598

679	56.67	11.075	19.9946	0.0149513	0.332799	293.15	293.15	0	329.909	329.909	0.074865	0.0748196

680	56.5	11.0616	20.0008	0.014934	0.331601	293.15	293.15	0	329.738	329.738	0.0748253	0.0747803

681	56.33	11.0498	20.0008	0.0149187	0.324391	293.15	293.15	0	329.572	329.572	0.0747866	0.0747413

682	56.17	10.9958	20.0008	0.0148466	0.317659	293.15	293.15	0	329.406	329.406	0.0747479	0.0747029

683	56.03	14.2957	20.0008	0.0193029	0.238513	293.15	293.15	0	329.246	329.246	0.0747419	0.0746695

684	55.99	28.9457	20.0008	0.0390848	0.0998615	293.15	293.15	0	329.077	329.077	0.0747764	0.0746609

685	55.92	45.4104	20.0008	0.0613179	0.00750948	293.15	293.15	0	328.905	328.905	0.0747768	0.0746455

686	55.77	58.6591	20.0008	0.0792114	-0.0453581	293.15	293.15	0	328.735	328.735	0.07475	0.0746094

687	55.59	68.9164	20.0008	0.0930674	-0.091181	293.15	293.15	0	328.568	328.568	0.074717	0.0745678

688	55.43	76.9546	20.0008	0.103927	-0.139496	293.15	293.15	0	328.402	328.402	0.0746857	0.0745307

689	55.28	83.5768	20.0008	0.112876	-0.194186	293.15	293.15	0	328.247	328.247	0.074656	0.0744956

690	55.15	88.9106	20.0008	0.120084	-0.253603	293.15	293.15	0	328.079	328.079	0.0746288	0.0744641

691	55.02	92.9157	20.0008	0.125499	-0.312098	293.15	293.15	0	327.91	327.91	0.0745989	0.0744329

692	54.88	95.6751	20.0008	0.129231	-0.373365	293.15	293.15	0	327.737	327.737	0.0745687	0.0744009

693	54.75	97.5684	20.0008	0.131794	-0.429313	293.15	293.15	0	327.587	327.587	0.0745384	0.0743705

694	54.62	98.888	20.0008	0.133582	-0.49519	293.15	293.15	0	327.415	327.415	0.0745091	0.0743402

695	54.5	99.6981	20.0008	0.134681	-0.565096	293.15	293.15	0	327.242	327.242	0.0744803	0.0743104

696	54.37	100.169	20.0008	0.135323	-0.630988	293.15	293.15	0	327.076	327.076	0.0744503	0.0742808

697	54.24	100.485	20.0008	0.135755	-0.704108	293.15	293.15	0	326.904	326.904	0.0744204	0.0742512

698	54.12	100.661	20.0008	0.135998	-0.777063	293.15	293.15	0	326.739	326.739	0.0743914	0.0742223

699	54	100.611	20.0008	0.135935	-0.844866	293.15	293.15	0	326.584	326.584	0.0743618	0.0741936

700	53.87	100.311	20.0008	0.135535	-0.921136	293.15	293.15	0	326.41	326.41	0.0743318	0.0741643

701	53.75	99.8058	20.0008	0.134857	-0.996084	293.15	293.15	0	326.247	326.247	0.0743009	0.0741347

702	53.62	99.1962	20.0008	0.134039	-1.0734	293.15	293.15	0	326.074	326.074	0.0742696	0.0741048

703	53.49	98.4406	20.0008	0.133023	-1.15459	293.15	293.15	0	325.892	325.892	0.0742374	0.0740744

704	53.36	97.4937	20.0008	0.131749	-1.22486	293.15	293.15	0	325.734	325.734	0.074205	0.0740436

705	53.23	96.3249	20.0008	0.130174	-1.30275	293.15	293.15	0	325.571	325.571	0.0741718	0.074013

706	53.09	94.9602	19.9914	0.128336	-1.37351	293.15	293.15	0	325.408	325.408	0.074137	0.0739799

707	52.95	93.5198	19.9904	0.126394	-1.44594	293.15	293.15	0	325.25	325.25	0.0741025	0.0739476

708	52.8	91.9735	19.9987	0.12431	-1.52185	293.15	293.15	0	325.076	325.076	0.0740663	0.0739134

709	52.65	90.2961	20.0008	0.122048	-1.59358	293.15	293.15	0	324.907	324.907	0.0740288	0.0738781

710	52.5	88.5227	19.9987	0.119657	-1.66824	293.15	293.15	0	324.734	324.734	0.0739893	0.0738418

711	52.34	86.59	19.9904	0.11705	-1.73036	293.15	293.15	0	324.574	324.574	0.0739487	0.0738034

712	52.17	84.4785	19.9904	0.114202	-1.79037	293.15	293.15	0	324.406	324.406	0.0739058	0.0737638

713	52	82.1412	19.9904	0.111048	-1.84802	293.15	293.15	0	324.243	324.243	0.0738622	0.0737241

714	51.82	79.5685	19.9966	0.107576	-1.9039	293.15	293.15	0	324.07	324.07	0.0738155	0.0736814

715	51.63	76.7662	20.0008	0.103793	-1.95275	293.15	293.15	0	323.904	323.904	0.0737675	0.0736371

716	51.43	73.6604	20.0008	0.0995997	-1.99162	293.15	293.15	0	323.743	323.743	0.0737155	0.07359

717	51.22	70.1796	19.9956	0.0948993	-2.02459	293.15	293.15	0	323.585	323.585	0.0736607	0.0735409

718	50.99	66.2523	19.9956	0.0895947	-2.04976	293.15	293.15	0	323.412	323.412	0.0736029	0.0734884

719	50.75	61.863	20.0008	0.083665	-2.0606	293.15	293.15	0	323.248	323.248	0.0735406	0.0734322

720	50.51	57.3622	20.0008	0.0775839	-2.05999	293.15	293.15	0	323.075	323.075	0.0734755	0.0733744

721	50.24	52.5505	20.0008	0.0710815	-2.04618	293.15	293.15	0	322.902	322.902	0.0734065	0.0733122

722	49.97	47.5541	20.0008	0.0643287	-2.02776	293.15	293.15	0	322.738	322.738	0.0733343	0.0732469

723	49.68	42.7742	19.9966	0.0578677	-2.00133	293.15	293.15	0	322.581	322.581	0.0732616	0.0731792

724	49.38	38.3733	19.9946	0.0519186	-1.96047	293.15	293.15	0	322.41	322.41	0.073188	0.07311

725	49.09	34.5424	20.0008	0.0467397	-1.91622	293.15	293.15	0	322.244	322.244	0.0731145	0.07304

726	48.79	31.428	20.0008	0.0425294	-1.87012	293.15	293.15	0	322.071	322.071	0.0730429	0.0729699

727	48.49	28.8927	19.9966	0.0391021	-1.8203	293.15	293.15	0	321.907	321.907	0.072972	0.0729007

728	48.2	26.8789	19.9998	0.0363798	-1.76028	293.15	293.15	0	321.735	321.735	0.0729024	0.0728323

729	47.91	25.2936	19.9977	0.0342373	-1.70583	293.15	293.15	0	321.586	321.586	0.0728335	0.0727644

730	47.63	24.0561	19.9987	0.0325649	-1.64184	293.15	293.15	0	321.412	321.412	0.0727658	0.0726978

731	47.35	23.0447	20.0008	0.0311985	-1.57779	293.15	293.15	0	321.243	321.243	0.0726996	0.0726316

732	47.07	22.2323	19.9977	0.0301011	-1.50669	293.15	293.15	0	321.075	321.075	0.0726341	0.0725666

733	46.8	21.6027	19.9987	0.0292511	-1.43137	293.15	293.15	0	320.902	320.902	0.0725699	0.0725024

734	46.53	21.1185	19.9925	0.0285979	-1.35431	293.15	293.15	0	320.733	320.733	0.0725056	0.0724384

735	46.27	20.6741	19.9925	0.0279983	-1.28296	293.15	293.15	0	320.581	320.581	0.0724426	0.0723762

736	46.01	20.2023	20.0008	0.0273616	-1.19505	293.15	293.15	0	320.408	320.408	0.0723805	0.0723153

737	45.75	19.7344	20.0008	0.0267299	-1.10817	293.15	293.15	0	320.244	320.244	0.0723201	0.0722547

738	45.5	19.2261	20.0008	0.0260435	-1.02488	293.15	293.15	0	320.076	320.076	0.0722597	0.072195

739	45.25	18.7374	19.9935	0.0253834	-0.925134	293.15	293.15	0	319.897	319.897	0.0722003	0.0721362

740	44.99	18.3461	19.9977	0.0248552	-0.834778	293.15	293.15	0	319.739	319.739	0.0721415	0.072077

741	44.75	18.0241	20.0008	0.0244208	-0.740952	293.15	293.15	0	319.577	319.577	0.0720837	0.0720193

742	44.51	17.7161	20.0008	0.0240053	-0.649369	293.15	293.15	0	319.413	319.413	0.0720276	0.0719625

743	44.27	17.3941	20.0008	0.0235706	-0.546348	293.15	293.15	0	319.24	319.24	0.0719716	0.0719065

744	44.04	17.0471	20.0008	0.0231021	-0.445592	293.15	293.15	0	319.073	319.073	0.0719158	0.0718512

745	43.81	16.7373	20.0008	0.0226838	-0.339219	293.15	293.15	0	318.902	318.902	0.0718622	0.0717973

746	43.58	16.4375	20.0008	0.022279	-0.240018	293.15	293.15	0	318.736	318.736	0.0718078	0.0717435

747	43.35	16.1936	20.0008	0.02195	-0.138077	293.15	293.15	0	318.581	318.581	0.0717546	0.0716903

748	43.14	15.9704	19.9956	0.0216488	-0.0278225	293.15	293.15	0	318.409	318.409	0.0717028	0.0716392

749	42.92	15.7163	19.9956	0.0213058	0.0791376	293.15	293.15	0	318.244	318.244	0.0716519	0.0715885

750	42.74	15.4255	20.0008	0.0209128	0.166754	293.15	293.15	0	318.071	318.071	0.0716104	0.0715465

751	42.65	14.5862	20.0008	0.0197754	0.226781	293.15	293.15	0	317.908	317.908	0.0715851	0.0715252

752	42.62	12.8537	20.0008	0.0174267	0.25937	293.15	293.15	0	317.741	317.741	0.0715736	0.0715185

753	42.62	10.4515	20.0008	0.0141698	0.275497	293.15	293.15	0	317.579	317.579	0.0715685	0.0715172

754	42.62	7.94162	20.0008	0.010767	0.279958	293.15	293.15	0	317.413	317.413	0.0715669	0.0715186

755	42.64	5.6014	20.0008	0.00759418	0.273365	293.15	293.15	0	317.24	317.24	0.0715674	0.0715222

756	42.65	3.62973	20.0008	0.00492104	0.260154	293.15	293.15	0	317.069	317.069	0.0715674	0.0715242

757	42.64	2.08777	20.0008	0.00283053	0.244765	293.15	293.15	0	316.903	316.903	0.0715646	0.0715218

758	42.62	1.07351	20.0008	0.00145544	0.226039	293.15	293.15	0	316.739	316.739	0.07156	0.0715173

759	42.58	0.517258	20.0008	0.000701292	0.207547	293.15	293.15	0	316.582	316.582	0.0715523	0.071509

760	42.54	0.366925	20.0008	0.00049748	0.18663	293.15	293.15	0	316.412	316.412	0.0715412	0.071498

761	42.47	0.577708	20.0008	0.000783277	0.168051	293.15	293.15	0	316.244	316.244	0.071527	0.0714823

762	42.39	1.04029	20.0008	0.0014105	0.146992	293.15	293.15	0	316.066	316.066	0.0715098	0.0714636

763	42.3	1.62185	20.0008	0.00219908	0.131313	293.15	293.15	0	315.898	315.898	0.0714886	0.0714414

764	42.19	2.37328	20.0008	0.00321806	0.119293	293.15	293.15	0	315.744	315.744	0.0714642	0.0714152

765	42.07	3.19671	20.0008	0.00433474	0.105142	293.15	293.15	0	315.577	315.577	0.0714382	0.0713874

766	41.95	3.96795	20.0008	0.00538074	0.0912046	293.15	293.15	0	315.41	315.41	0.0714101	0.0713591

767	41.82	4.75278	20.0008	0.00644527	0.0797926	293.15	293.15	0	315.24	315.24	0.0713805	0.0713282

768	41.67	5.49637	20.0008	0.00745398	0.0709795	293.15	293.15	0	315.067	315.067	0.0713488	0.0712946

769	41.53	6.2419	20.0008	0.00846542	0.0652746	293.15	293.15	0	314.917	314.917	0.0713148	0.0712597

770	41.38	6.92433	20.0008	0.00939137	0.0558637	293.15	293.15	0	314.747	314.747	0.0712809	0.0712248

771	41.22	7.49211	20.0008	0.0101619	0.047706	293.15	293.15	0	314.58	314.58	0.0712448	0.0711882

772	41.07	8.00637	19.9904	0.01086	0.040952	293.15	293.15	0	314.408	314.408	0.0712086	0.0711508

773	40.9	8.45461	19.9956	0.0114685	0.0385108	293.15	293.15	0	314.243	314.243	0.0711712	0.0711126

774	40.74	8.91043	20.0008	0.0120874	0.0324513	293.15	293.15	0	314.069	314.069	0.071133	0.0710747

775	40.58	9.29623	20.0008	0.0126114	0.0295468	293.15	293.15	0	313.896	313.896	0.0710946	0.071036

776	40.41	9.65987	20.0008	0.0131054	0.0285559	293.15	293.15	0	313.741	313.741	0.0710554	0.0709956

777	40.24	9.97773	20.0008	0.0135374	0.0284129	293.15	293.15	0	313.576	313.576	0.0710156	0.0709559

778	40.08	10.177	20.0008	0.0138084	0.0266247	293.15	293.15	0	313.404	313.404	0.0709775	0.0709183

779	39.91	10.2341	20.0008	0.0138866	0.0213138	293.15	293.15	0	313.239	313.239	0.0709378	0.0708783

780	39.74	10.2555	20.0008	0.0139164	0.0212632	293.15	293.15	0	313.075	313.075	0.0708988	0.070839

781	39.57	10.2203	19.9914	0.0138693	0.0212779	293.15	293.15	0	312.901	312.901	0.0708582	0.0707989

782	39.41	10.2269	19.9904	0.0138789	0.0175593	293.15	293.15	0	312.739	312.739	0.0708198	0.0707603

783	39.24	10.2438	19.9987	0.0139026	0.0132302	293.15	293.15	0	312.58	312.58	0.0707817	0.0707209

784	39.08	10.2449	19.9925	0.0139047	0.00939058	293.15	293.15	0	312.408	312.408	0.0707422	0.0706818

785	38.92	10.3073	19.9904	0.0139901	0.00625306	293.15	293.15	0	312.244	312.244	0.0707045	0.0706437

786	38.75	10.3781	19.9904	0.014087	0.00015125	293.15	293.15	0	312.074	312.074	0.0706653	0.0706046

787	38.59	10.3894	19.9987	0.0141029	-0.00633198	293.15	293.15	0	311.906	311.906	0.0706277	0.0705665

788	38.44	10.2981	20.0008	0.0139798	-0.0138358	293.15	293.15	0	311.74	311.74	0.0705906	0.0705303

789	38.28	10.1893	20.0008	0.0138326	-0.0203914	293.15	293.15	0	311.582	311.582	0.0705539	0.0704931

790	38.13	10.0699	19.9935	0.0136711	-0.0314305	293.15	293.15	0	311.412	311.412	0.0705181	0.0704578

791	37.98	9.90932	19.9925	0.0134538	-0.0452726	293.15	293.15	0	311.238	311.238	0.0704829	0.0704227

792	37.84	9.7114	20.0008	0.0131857	-0.0581437	293.15	293.15	0	311.071	311.071	0.0704483	0.0703882

793	37.69	9.49306	19.9987	0.0128898	-0.0727797	293.15	293.15	0	310.902	310.902	0.0704137	0.0703533

794	37.55	9.32784	19.9904	0.012666	-0.0926277	293.15	293.15	0	310.736	310.736	0.0703795	0.0703197

795	37.41	9.22879	19.9966	0.0125321	-0.108932	293.15	293.15	0	310.579	310.579	0.0703459	0.0702867

796	37.26	9.1079	19.9998	0.0123684	-0.128576	293.15	293.15	0	310.407	310.407	0.0703119	0.0702531

797	37.13	8.94896	19.9904	0.0121531	-0.154424	293.15	293.15	0	310.234	310.234	0.0702793	0.0702207

798	36.99	8.78573	19.9966	0.0119319	-0.178286	293.15	293.15	0	310.076	310.076	0.0702476	0.0701884

799	36.85	8.61746	20.0008	0.0117039	-0.203437	293.15	293.15	0	309.914	309.914	0.0702148	0.0701555

800	36.72	8.48057	20.0008	0.0115184	-0.235602	293.15	293.15	0	309.74	309.74	0.0701843	0.070125

801	36.59	8.33375	20.0008	0.0113195	-0.267018	293.15	293.15	0	309.577	309.577	0.0701537	0.0700946

802	36.46	8.20367	19.9956	0.0111432	-0.303572	293.15	293.15	0	309.403	309.403	0.0701226	0.0700634

803	36.33	8.06423	20.0008	0.0109542	-0.338093	293.15	293.15	0	309.239	309.239	0.0700922	0.0700336

804	36.21	7.89484	20.0008	0.0107246	-0.37832	293.15	293.15	0	309.067	309.067	0.0700628	0.0700034

805	36.09	7.68492	20.0008	0.0104398	-0.415719	293.15	293.15	0	308.919	308.919	0.0700343	0.069975

806	35.96	7.51825	20.0008	0.0102138	-0.460705	293.15	293.15	0	308.745	308.745	0.0700047	0.0699457

807	35.85	7.34714	20.0008	0.00998165	-0.513149	293.15	293.15	0	308.574	308.574	0.069977	0.0699182

808	35.73	7.18578	20.0008	0.00976278	-0.561013	293.15	293.15	0	308.408	308.408	0.0699488	0.0698899

809	35.61	7.10306	20.0008	0.00965074	-0.614847	293.15	293.15	0	308.234	308.234	0.0699205	0.0698625

810	35.49	7.06119	20.0008	0.0095942	-0.670465	293.15	293.15	0	308.071	308.071	0.069893	0.0698346

811	35.38	7.00777	20.0008	0.00952193	-0.726037	293.15	293.15	0	307.917	307.917	0.0698669	0.0698085

812	35.27	6.95224	20.0008	0.00944681	-0.793097	293.15	293.15	0	307.741	307.741	0.0698402	0.0697816

813	35.16	6.82998	20.0008	0.009281	-0.856988	293.15	293.15	0	307.576	307.576	0.0698142	0.0697552

814	35.05	6.67898	19.9925	0.00907611	-0.925757	293.15	293.15	0	307.407	307.407	0.0697882	0.0697294

815	34.94	6.51675	19.9987	0.00885595	-0.9988	293.15	293.15	0	307.239	307.239	0.0697625	0.0697033

816	34.83	6.38596	20.0008	0.00867849	-1.0768	293.15	293.15	0	307.066	307.066	0.069737	0.0696781

817	34.73	6.31925	20.0008	0.00858811	-1.14737	293.15	293.15	0	306.919	306.919	0.0697126	0.0696537

818	34.63	6.27891	19.9956	0.00853355	-1.23002	293.15	293.15	0	306.751	306.751	0.069688	0.0696296

819	34.52	6.15157	20.0008	0.00836075	-1.31545	293.15	293.15	0	306.581	306.581	0.0696637	0.0696054

820	34.43	5.98046	20.0008	0.00812843	-1.40713	293.15	293.15	0	306.408	306.408	0.0696398	0.0695824

821	34.33	5.83579	19.9935	0.00793204	-1.50035	293.15	293.15	0	306.241	306.241	0.0696168	0.0695588

822	34.23	5.76555	19.9904	0.00783681	-1.60039	293.15	293.15	0	306.07	306.07	0.0695938	0.0695352

823	34.13	5.70119	19.9966	0.00774954	-1.69305	293.15	293.15	0	305.914	305.914	0.0695705	0.0695132

824	34.04	5.50866	19.9998	0.00748805	-1.79612	293.15	293.15	0	305.748	305.748	0.069548	0.0694919

825	33.95	5.30253	19.9904	0.00720806	-1.91472	293.15	293.15	0	305.567	305.567	0.0695265	0.0694689

826	33.85	5.21648	19.9904	0.0070913	-2.01997	293.15	293.15	0	305.41	305.41	0.0695048	0.0694464

827	33.76	5.17483	19.9904	0.00703488	-2.13419	293.15	293.15	0	305.247	305.247	0.069483	0.0694245

828	33.67	5.13985	20.0008	0.00698752	-2.25014	293.15	293.15	0	305.083	305.083	0.0694612	0.0694036

829	33.58	5.15955	20.0008	0.00701449	-2.37726	293.15	293.15	0	304.91	304.91	0.0694402	0.0693822

830	33.49	5.14586	20.0008	0.00699607	-2.5033	293.15	293.15	0	304.745	304.745	0.0694189	0.0693606

831	33.41	5.04638	20.0008	0.00686099	-2.63936	293.15	293.15	0	304.572	304.572	0.0693987	0.0693412

832	33.32	4.91084	20.0008	0.00667688	-2.78102	293.15	293.15	0	304.399	304.399	0.0693786	0.0693217

833	33.24	4.79324	20.0008	0.00651716	-2.91218	293.15	293.15	0	304.242	304.242	0.0693588	0.0693018

834	33.16	4.67379	20.0102	0.00635492	-3.06063	293.15	293.15	0	304.071	304.071	0.0693391	0.069282

835	33.08	4.54647	20.0029	0.00618195	-3.20923	293.15	293.15	0	303.904	303.904	0.0693201	0.0692628

836	33	4.38151	19.9998	0.0059578	-3.36228	293.15	293.15	0	303.74	303.74	0.0693009	0.0692437

837	32.92	4.33152	20.0008	0.00588997	-3.5081	293.15	293.15	0	303.585	303.585	0.0692822	0.0692247

838	32.84	4.28587	20.0008	0.00582803	-3.67368	293.15	293.15	0	303.415	303.415	0.0692641	0.0692068

839	32.76	4.2171	20.0008	0.00573465	-3.85161	293.15	293.15	0	303.238	303.238	0.0692459	0.0691877
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		cm-1		%T

		4000		98.07

		3999		98.07

		3998		98.07

		3997		98.07

		3996		98.07

		3995		98.07

		3994		98.07

		3993		98.06

		3992		98.06

		3991		98.06

		3990		98.06

		3989		98.06

		3988		98.05

		3987		98.05

		3986		98.05

		3985		98.05

		3984		98.05

		3983		98.05

		3982		98.05

		3981		98.05

		3980		98.05

		3979		98.05

		3978		98.05

		3977		98.05

		3976		98.05

		3975		98.05

		3974		98.05

		3973		98.06

		3972		98.06

		3971		98.06

		3970		98.06

		3969		98.06

		3968		98.06

		3967		98.06

		3966		98.06

		3965		98.06

		3964		98.06

		3963		98.06

		3962		98.06

		3961		98.06

		3960		98.06

		3959		98.06

		3958		98.06

		3957		98.07

		3956		98.07

		3955		98.06

		3954		98.06

		3953		98.06

		3952		98.06

		3951		98.06

		3950		98.06

		3949		98.06

		3948		98.06

		3947		98.06

		3946		98.06

		3945		98.05

		3944		98.05

		3943		98.05

		3942		98.05

		3941		98.05

		3940		98.05

		3939		98.05

		3938		98.06

		3937		98.06

		3936		98.06

		3935		98.06

		3934		98.06

		3933		98.06

		3932		98.06

		3931		98.06

		3930		98.06

		3929		98.06

		3928		98.06

		3927		98.06

		3926		98.06

		3925		98.06

		3924		98.05

		3923		98.05

		3922		98.04

		3921		98.04

		3920		98.03

		3919		98.03

		3918		98.03

		3917		98.02

		3916		98.02

		3915		98.02

		3914		98.02

		3913		98.02

		3912		98.02

		3911		98.02

		3910		98.02

		3909		98.02

		3908		98.02

		3907		98.02

		3906		98.02

		3905		98.02

		3904		98.02

		3903		98.01

		3902		98.01

		3901		98.01

		3900		98.01

		3899		98.01

		3898		98.01

		3897		98.01

		3896		98.01

		3895		98.01

		3894		98.01

		3893		98.01

		3892		98.01

		3891		98.01

		3890		98.01

		3889		98.01

		3888		98

		3887		98

		3886		98

		3885		98

		3884		98

		3883		98

		3882		98

		3881		98

		3880		98

		3879		98

		3878		98

		3877		98

		3876		98

		3875		98

		3874		98

		3873		98

		3872		98

		3871		98

		3870		98

		3869		98

		3868		98

		3867		98

		3866		98

		3865		98

		3864		98.01

		3863		98.01

		3862		98.01

		3861		98.01

		3860		98.01

		3859		98.01

		3858		98.01

		3857		98.01

		3856		98.02

		3855		98.01

		3854		98.01

		3853		98.01

		3852		98.01

		3851		98.01

		3850		98.01

		3849		98.01

		3848		98

		3847		98

		3846		98

		3845		98

		3844		98

		3843		98

		3842		97.99

		3841		97.99

		3840		97.99

		3839		97.99

		3838		97.99

		3837		97.99

		3836		97.99

		3835		97.99

		3834		97.99

		3833		97.99

		3832		97.99

		3831		97.99

		3830		98

		3829		98

		3828		98

		3827		98

		3826		98.01

		3825		98.01

		3824		98.01

		3823		98.01

		3822		98.01

		3821		98.01

		3820		98.01

		3819		98.01

		3818		98.01

		3817		98.02

		3816		98.02

		3815		98.02

		3814		98.02

		3813		98.02

		3812		98.02

		3811		98.02

		3810		98.02

		3809		98.02

		3808		98.02

		3807		98.02

		3806		98.02

		3805		98.02

		3804		98.02

		3803		98.02

		3802		98.02

		3801		98.02

		3800		98.02

		3799		98.02

		3798		98.02

		3797		98.03

		3796		98.03

		3795		98.03

		3794		98.03

		3793		98.03

		3792		98.03

		3791		98.04

		3790		98.04

		3789		98.04

		3788		98.04

		3787		98.05

		3786		98.05

		3785		98.05

		3784		98.05

		3783		98.06

		3782		98.06

		3781		98.06

		3780		98.06

		3779		98.06

		3778		98.06

		3777		98.06

		3776		98.06

		3775		98.06

		3774		98.06

		3773		98.05

		3772		98.05

		3771		98.05

		3770		98.05

		3769		98.04

		3768		98.04

		3767		98.04

		3766		98.04

		3765		98.04

		3764		98.04

		3763		98.04

		3762		98.04

		3761		98.03

		3760		98.03

		3759		98.03

		3758		98.02

		3757		98.02

		3756		98.01

		3755		98

		3754		98

		3753		97.99

		3752		97.98

		3751		97.98

		3750		97.97

		3749		97.97

		3748		97.97

		3747		97.97

		3746		97.97

		3745		97.97

		3744		97.97

		3743		97.97

		3742		97.98

		3741		97.98

		3740		97.98

		3739		97.98

		3738		97.99

		3737		97.99

		3736		97.99

		3735		97.99

		3734		97.99

		3733		98

		3732		98

		3731		98

		3730		98

		3729		98

		3728		97.99

		3727		97.99

		3726		97.99

		3725		97.99

		3724		97.99

		3723		97.98

		3722		97.98

		3721		97.97

		3720		97.97

		3719		97.96

		3718		97.95

		3717		97.94

		3716		97.93

		3715		97.92

		3714		97.91

		3713		97.9

		3712		97.89

		3711		97.88

		3710		97.87

		3709		97.86

		3708		97.86

		3707		97.85

		3706		97.84

		3705		97.84

		3704		97.83

		3703		97.82

		3702		97.81

		3701		97.79

		3700		97.78

		3699		97.77

		3698		97.75

		3697		97.74

		3696		97.72

		3695		97.71

		3694		97.7

		3693		97.68

		3692		97.67

		3691		97.66

		3690		97.65

		3689		97.64

		3688		97.63

		3687		97.62

		3686		97.6

		3685		97.59

		3684		97.58

		3683		97.56

		3682		97.55

		3681		97.54

		3680		97.52

		3679		97.51

		3678		97.5

		3677		97.49

		3676		97.48

		3675		97.47

		3674		97.47

		3673		97.47

		3672		97.47

		3671		97.47

		3670		97.47

		3669		97.47

		3668		97.47

		3667		97.48

		3666		97.48

		3665		97.48

		3664		97.49

		3663		97.49

		3662		97.5

		3661		97.5

		3660		97.51

		3659		97.52

		3658		97.53

		3657		97.54

		3656		97.55

		3655		97.56

		3654		97.57

		3653		97.59

		3652		97.6

		3651		97.62

		3650		97.63

		3649		97.65

		3648		97.67

		3647		97.68

		3646		97.7

		3645		97.72

		3644		97.74

		3643		97.76

		3642		97.77

		3641		97.79

		3640		97.81

		3639		97.82

		3638		97.83

		3637		97.85

		3636		97.86

		3635		97.87

		3634		97.87

		3633		97.88

		3632		97.89

		3631		97.89

		3630		97.9

		3629		97.9

		3628		97.91

		3627		97.92

		3626		97.93

		3625		97.94

		3624		97.94

		3623		97.95

		3622		97.96

		3621		97.96

		3620		97.96

		3619		97.96

		3618		97.96

		3617		97.96

		3616		97.95

		3615		97.94

		3614		97.94

		3613		97.93

		3612		97.93

		3611		97.92

		3610		97.92

		3609		97.92

		3608		97.92

		3607		97.92

		3606		97.92

		3605		97.93

		3604		97.94

		3603		97.95

		3602		97.96

		3601		97.97

		3600		97.98

		3599		97.98

		3598		97.99

		3597		98

		3596		98

		3595		98.01

		3594		98.01

		3593		98.02

		3592		98.02

		3591		98.02

		3590		98.03

		3589		98.03

		3588		98.04

		3587		98.04

		3586		98.05

		3585		98.05

		3584		98.06

		3583		98.06

		3582		98.06

		3581		98.07

		3580		98.07

		3579		98.07

		3578		98.07

		3577		98.07

		3576		98.07

		3575		98.07

		3574		98.07

		3573		98.07

		3572		98.07

		3571		98.07

		3570		98.07

		3569		98.07

		3568		98.07

		3567		98.07

		3566		98.07

		3565		98.06

		3564		98.06

		3563		98.06

		3562		98.06

		3561		98.06

		3560		98.06

		3559		98.06

		3558		98.06

		3557		98.06

		3556		98.06

		3555		98.06

		3554		98.06

		3553		98.05

		3552		98.05

		3551		98.05

		3550		98.05

		3549		98.05

		3548		98.04

		3547		98.04

		3546		98.04

		3545		98.04

		3544		98.04

		3543		98.04

		3542		98.04

		3541		98.04

		3540		98.04

		3539		98.04

		3538		98.04

		3537		98.04

		3536		98.04

		3535		98.04

		3534		98.04

		3533		98.04

		3532		98.04

		3531		98.04

		3530		98.04

		3529		98.04

		3528		98.04

		3527		98.04

		3526		98.04

		3525		98.04

		3524		98.04

		3523		98.04

		3522		98.04

		3521		98.04

		3520		98.04

		3519		98.04

		3518		98.04

		3517		98.04

		3516		98.03

		3515		98.03

		3514		98.03

		3513		98.03

		3512		98.03

		3511		98.03

		3510		98.03

		3509		98.03

		3508		98.03

		3507		98.03

		3506		98.03

		3505		98.02

		3504		98.02

		3503		98.02

		3502		98.02

		3501		98.02

		3500		98.02

		3499		98.02

		3498		98.02

		3497		98.02

		3496		98.02

		3495		98.02

		3494		98.02

		3493		98.02

		3492		98.02

		3491		98.02

		3490		98.02

		3489		98.02

		3488		98.02

		3487		98.02

		3486		98.02

		3485		98.02

		3484		98.01

		3483		98.01

		3482		98.01

		3481		98.01

		3480		98.01

		3479		98.01

		3478		98.01

		3477		98

		3476		98

		3475		98

		3474		98

		3473		98

		3472		98

		3471		98

		3470		98

		3469		98

		3468		98

		3467		98

		3466		97.99

		3465		97.99

		3464		97.99

		3463		97.98

		3462		97.98

		3461		97.98

		3460		97.97

		3459		97.97

		3458		97.96

		3457		97.96

		3456		97.96

		3455		97.96

		3454		97.95

		3453		97.95

		3452		97.95

		3451		97.95

		3450		97.95

		3449		97.95

		3448		97.95

		3447		97.94

		3446		97.94

		3445		97.94

		3444		97.94

		3443		97.94

		3442		97.94

		3441		97.94

		3440		97.94

		3439		97.94

		3438		97.94

		3437		97.94

		3436		97.93

		3435		97.93

		3434		97.92

		3433		97.92

		3432		97.91

		3431		97.9

		3430		97.89

		3429		97.88

		3428		97.87

		3427		97.86

		3426		97.85

		3425		97.84

		3424		97.83

		3423		97.82

		3422		97.81

		3421		97.81

		3420		97.8

		3419		97.8

		3418		97.8

		3417		97.79

		3416		97.79

		3415		97.79

		3414		97.79

		3413		97.79

		3412		97.78

		3411		97.78

		3410		97.78

		3409		97.78

		3408		97.78

		3407		97.78

		3406		97.78

		3405		97.78

		3404		97.78

		3403		97.79

		3402		97.79

		3401		97.79

		3400		97.79

		3399		97.79

		3398		97.79

		3397		97.78

		3396		97.78

		3395		97.77

		3394		97.76

		3393		97.75

		3392		97.74

		3391		97.72

		3390		97.71

		3389		97.7

		3388		97.68

		3387		97.67

		3386		97.66

		3385		97.66

		3384		97.65

		3383		97.65

		3382		97.64

		3381		97.65

		3380		97.65

		3379		97.65

		3378		97.66

		3377		97.67

		3376		97.67

		3375		97.68

		3374		97.69

		3373		97.7

		3372		97.71

		3371		97.71

		3370		97.71

		3369		97.71

		3368		97.71

		3367		97.71

		3366		97.7

		3365		97.69

		3364		97.68

		3363		97.66

		3362		97.65

		3361		97.64

		3360		97.63

		3359		97.63

		3358		97.62

		3357		97.62

		3356		97.61

		3355		97.61

		3354		97.61

		3353		97.61

		3352		97.61

		3351		97.61

		3350		97.61

		3349		97.6

		3348		97.6

		3347		97.6

		3346		97.59

		3345		97.59

		3344		97.58

		3343		97.57

		3342		97.57

		3341		97.56

		3340		97.55

		3339		97.55

		3338		97.54

		3337		97.53

		3336		97.52

		3335		97.52

		3334		97.51

		3333		97.5

		3332		97.5

		3331		97.49

		3330		97.49

		3329		97.48

		3328		97.48

		3327		97.48

		3326		97.47

		3325		97.47

		3324		97.47

		3323		97.46

		3322		97.46

		3321		97.46

		3320		97.45

		3319		97.45

		3318		97.45

		3317		97.45

		3316		97.45

		3315		97.45

		3314		97.45

		3313		97.45

		3312		97.45

		3311		97.45

		3310		97.45

		3309		97.46

		3308		97.45

		3307		97.45

		3306		97.45

		3305		97.45

		3304		97.44

		3303		97.43

		3302		97.43

		3301		97.42

		3300		97.41

		3299		97.4

		3298		97.4

		3297		97.39

		3296		97.38

		3295		97.37

		3294		97.36

		3293		97.35

		3292		97.34

		3291		97.33

		3290		97.32

		3289		97.31

		3288		97.3

		3287		97.29

		3286		97.28

		3285		97.27

		3284		97.26

		3283		97.25

		3282		97.24

		3281		97.23

		3280		97.23

		3279		97.22

		3278		97.21

		3277		97.2

		3276		97.19

		3275		97.18

		3274		97.17

		3273		97.16

		3272		97.15

		3271		97.14

		3270		97.13

		3269		97.12

		3268		97.11

		3267		97.09

		3266		97.08

		3265		97.07

		3264		97.06

		3263		97.05

		3262		97.03

		3261		97.02

		3260		97.01

		3259		97

		3258		96.99

		3257		96.97

		3256		96.96

		3255		96.95

		3254		96.93

		3253		96.92

		3252		96.9

		3251		96.89

		3250		96.88

		3249		96.86

		3248		96.85

		3247		96.83

		3246		96.82

		3245		96.8

		3244		96.79

		3243		96.77

		3242		96.76

		3241		96.74

		3240		96.72

		3239		96.71

		3238		96.69

		3237		96.68

		3236		96.66

		3235		96.65

		3234		96.63

		3233		96.61

		3232		96.6

		3231		96.58

		3230		96.56

		3229		96.54

		3228		96.52

		3227		96.5

		3226		96.49

		3225		96.47

		3224		96.45

		3223		96.43

		3222		96.41

		3221		96.39

		3220		96.37

		3219		96.35

		3218		96.34

		3217		96.32

		3216		96.3

		3215		96.29

		3214		96.27

		3213		96.25

		3212		96.24

		3211		96.22

		3210		96.2

		3209		96.19

		3208		96.17

		3207		96.15

		3206		96.13

		3205		96.11

		3204		96.09

		3203		96.08

		3202		96.06

		3201		96.04

		3200		96.02

		3199		96

		3198		95.99

		3197		95.97

		3196		95.95

		3195		95.94

		3194		95.92

		3193		95.9

		3192		95.89

		3191		95.87

		3190		95.86

		3189		95.84

		3188		95.82

		3187		95.81

		3186		95.79

		3185		95.77

		3184		95.75

		3183		95.74

		3182		95.72

		3181		95.7

		3180		95.69

		3179		95.67

		3178		95.65

		3177		95.64

		3176		95.62

		3175		95.61

		3174		95.59

		3173		95.57

		3172		95.56

		3171		95.54

		3170		95.52

		3169		95.51

		3168		95.49

		3167		95.47

		3166		95.45

		3165		95.43

		3164		95.41

		3163		95.39

		3162		95.36

		3161		95.34

		3160		95.32

		3159		95.3

		3158		95.28

		3157		95.25

		3156		95.23

		3155		95.21

		3154		95.18

		3153		95.16

		3152		95.13

		3151		95.11

		3150		95.08

		3149		95.06

		3148		95.03

		3147		95

		3146		94.97

		3145		94.95

		3144		94.92

		3143		94.89

		3142		94.86

		3141		94.83

		3140		94.8

		3139		94.77

		3138		94.73

		3137		94.7

		3136		94.67

		3135		94.64

		3134		94.61

		3133		94.57

		3132		94.54

		3131		94.51

		3130		94.47

		3129		94.44

		3128		94.41

		3127		94.38

		3126		94.34

		3125		94.31

		3124		94.28

		3123		94.24

		3122		94.21

		3121		94.18

		3120		94.14

		3119		94.11

		3118		94.08

		3117		94.04

		3116		94.01

		3115		93.97

		3114		93.94

		3113		93.9

		3112		93.87

		3111		93.83

		3110		93.8

		3109		93.76

		3108		93.72

		3107		93.69

		3106		93.65

		3105		93.62

		3104		93.59

		3103		93.55

		3102		93.52

		3101		93.49

		3100		93.46

		3099		93.43

		3098		93.4

		3097		93.37

		3096		93.34

		3095		93.31

		3094		93.29

		3093		93.26

		3092		93.24

		3091		93.21

		3090		93.19

		3089		93.16

		3088		93.14

		3087		93.11

		3086		93.09

		3085		93.07

		3084		93.04

		3083		93.02

		3082		93

		3081		92.98

		3080		92.95

		3079		92.93

		3078		92.91

		3077		92.89

		3076		92.86

		3075		92.84

		3074		92.82

		3073		92.79

		3072		92.77

		3071		92.74

		3070		92.72

		3069		92.69

		3068		92.66

		3067		92.64

		3066		92.61

		3065		92.58

		3064		92.55

		3063		92.52

		3062		92.49

		3061		92.46

		3060		92.43

		3059		92.39

		3058		92.36

		3057		92.32

		3056		92.28

		3055		92.25

		3054		92.21

		3053		92.16

		3052		92.12

		3051		92.08

		3050		92.03

		3049		91.99

		3048		91.94

		3047		91.89

		3046		91.84

		3045		91.79

		3044		91.74

		3043		91.68

		3042		91.63

		3041		91.57

		3040		91.51

		3039		91.45

		3038		91.39

		3037		91.32

		3036		91.26

		3035		91.19

		3034		91.13

		3033		91.06

		3032		90.99

		3031		90.93

		3030		90.86

		3029		90.8

		3028		90.73

		3027		90.67

		3026		90.61

		3025		90.55

		3024		90.49

		3023		90.43

		3022		90.37

		3021		90.31

		3020		90.25

		3019		90.2

		3018		90.14

		3017		90.09

		3016		90.04

		3015		89.99

		3014		89.94

		3013		89.89

		3012		89.84

		3011		89.79

		3010		89.75

		3009		89.71

		3008		89.67

		3007		89.63

		3006		89.59

		3005		89.55

		3004		89.52

		3003		89.48

		3002		89.45

		3001		89.42

		3000		89.39

		2999		89.35

		2998		89.32

		2997		89.28

		2996		89.24

		2995		89.2

		2994		89.15

		2993		89.1

		2992		89.05

		2991		89

		2990		88.94

		2989		88.89

		2988		88.84

		2987		88.79

		2986		88.73

		2985		88.68

		2984		88.62

		2983		88.56

		2982		88.49

		2981		88.42

		2980		88.33

		2979		88.22

		2978		88.09

		2977		87.92

		2976		87.71

		2975		87.45

		2974		87.12

		2973		86.73

		2972		86.27

		2971		85.74

		2970		85.16

		2969		84.54

		2968		83.89

		2967		83.21

		2966		82.53

		2965		81.87

		2964		81.22

		2963		80.62

		2962		80.06

		2961		79.56

		2960		79.13

		2959		78.76

		2958		78.47

		2957		78.25

		2956		78.12

		2955		78.07

		2954		78.11

		2953		78.23

		2952		78.42

		2951		78.65

		2950		78.89

		2949		79.13

		2948		79.33

		2947		79.48

		2946		79.55

		2945		79.54

		2944		79.43

		2943		79.23

		2942		78.93

		2941		78.57

		2940		78.14

		2939		77.67

		2938		77.18

		2937		76.67

		2936		76.15

		2935		75.63

		2934		75.09

		2933		74.52

		2932		73.9

		2931		73.21

		2930		72.43

		2929		71.52

		2928		70.48

		2927		69.27

		2926		67.89

		2925		66.33

		2924		64.63

		2923		62.8

		2922		60.9

		2921		59

		2920		57.16

		2919		55.47

		2918		54

		2917		52.83

		2916		52

		2915		51.57

		2914		51.53

		2913		51.9

		2912		52.63

		2911		53.68

		2910		54.98

		2909		56.45

		2908		58.04

		2907		59.66

		2906		61.26

		2905		62.79

		2904		64.22

		2903		65.54

		2902		66.73

		2901		67.79

		2900		68.75

		2899		69.6

		2898		70.38

		2897		71.09

		2896		71.75

		2895		72.38

		2894		72.97

		2893		73.54

		2892		74.11

		2891		74.66

		2890		75.2

		2889		75.74

		2888		76.28

		2887		76.8

		2886		77.3

		2885		77.78

		2884		78.21

		2883		78.6

		2882		78.92

		2881		79.17

		2880		79.35

		2879		79.46

		2878		79.5

		2877		79.49

		2876		79.44

		2875		79.36

		2874		79.27

		2873		79.2

		2872		79.15

		2871		79.13

		2870		79.14

		2869		79.17

		2868		79.2

		2867		79.22

		2866		79.19

		2865		79.09

		2864		78.89

		2863		78.56

		2862		78.06

		2861		77.36

		2860		76.45

		2859		75.29

		2858		73.9

		2857		72.31

		2856		70.56

		2855		68.7

		2854		66.81

		2853		64.97

		2852		63.29

		2851		61.86

		2850		60.78

		2849		60.12

		2848		59.93

		2847		60.24

		2846		61.02

		2845		62.21

		2844		63.74

		2843		65.54

		2842		67.49

		2841		69.52

		2840		71.53

		2839		73.45

		2838		75.24

		2837		76.84

		2836		78.25

		2835		79.48

		2834		80.54

		2833		81.44

		2832		82.22

		2831		82.89

		2830		83.48

		2829		83.99

		2828		84.44

		2827		84.84

		2826		85.2

		2825		85.52

		2824		85.81

		2823		86.08

		2822		86.33

		2821		86.55

		2820		86.76

		2819		86.96

		2818		87.14

		2817		87.3

		2816		87.46

		2815		87.61

		2814		87.75

		2813		87.87

		2812		88

		2811		88.11

		2810		88.22

		2809		88.33

		2808		88.43

		2807		88.52

		2806		88.62

		2805		88.71

		2804		88.8

		2803		88.88

		2802		88.96

		2801		89.04

		2800		89.12

		2799		89.2

		2798		89.27

		2797		89.33

		2796		89.4

		2795		89.46

		2794		89.52

		2793		89.57

		2792		89.63

		2791		89.68

		2790		89.72

		2789		89.77

		2788		89.81

		2787		89.85

		2786		89.89

		2785		89.92

		2784		89.95

		2783		89.99

		2782		90.02

		2781		90.05

		2780		90.07

		2779		90.1

		2778		90.12

		2777		90.15

		2776		90.17

		2775		90.2

		2774		90.22

		2773		90.24

		2772		90.26

		2771		90.28

		2770		90.3

		2769		90.33

		2768		90.35

		2767		90.37

		2766		90.39

		2765		90.42

		2764		90.44

		2763		90.46

		2762		90.49

		2761		90.51

		2760		90.54

		2759		90.56

		2758		90.59

		2757		90.61

		2756		90.63

		2755		90.66

		2754		90.68

		2753		90.7

		2752		90.73

		2751		90.75

		2750		90.78

		2749		90.8

		2748		90.82

		2747		90.85

		2746		90.87

		2745		90.9

		2744		90.92

		2743		90.95

		2742		90.97

		2741		90.99

		2740		91.01

		2739		91.03

		2738		91.05

		2737		91.07

		2736		91.09

		2735		91.1

		2734		91.11

		2733		91.13

		2732		91.14

		2731		91.15

		2730		91.16

		2729		91.17

		2728		91.19

		2727		91.2

		2726		91.21

		2725		91.22

		2724		91.23

		2723		91.23

		2722		91.23

		2721		91.23

		2720		91.22

		2719		91.21

		2718		91.2

		2717		91.17

		2716		91.15

		2715		91.12

		2714		91.09

		2713		91.05

		2712		91.02

		2711		90.98

		2710		90.94

		2709		90.91

		2708		90.87

		2707		90.84

		2706		90.81

		2705		90.78

		2704		90.75

		2703		90.73

		2702		90.7

		2701		90.68

		2700		90.66

		2699		90.64

		2698		90.62

		2697		90.6

		2696		90.58

		2695		90.55

		2694		90.53

		2693		90.5

		2692		90.48

		2691		90.45

		2690		90.42

		2689		90.39

		2688		90.37

		2687		90.34

		2686		90.32

		2685		90.3

		2684		90.28

		2683		90.26

		2682		90.25

		2681		90.24

		2680		90.23

		2679		90.22

		2678		90.22

		2677		90.22

		2676		90.22

		2675		90.22

		2674		90.22

		2673		90.22

		2672		90.22

		2671		90.23

		2670		90.23

		2669		90.23

		2668		90.24

		2667		90.24

		2666		90.24

		2665		90.24

		2664		90.24

		2663		90.24

		2662		90.24

		2661		90.24

		2660		90.24

		2659		90.24

		2658		90.23

		2657		90.23

		2656		90.23

		2655		90.22

		2654		90.22

		2653		90.22

		2652		90.22

		2651		90.22

		2650		90.23

		2649		90.23

		2648		90.24

		2647		90.25

		2646		90.27

		2645		90.28

		2644		90.29

		2643		90.31

		2642		90.32

		2641		90.33

		2640		90.34

		2639		90.35

		2638		90.36

		2637		90.37

		2636		90.37

		2635		90.37

		2634		90.38

		2633		90.38

		2632		90.39

		2631		90.39

		2630		90.4

		2629		90.42

		2628		90.44

		2627		90.46

		2626		90.48

		2625		90.51

		2624		90.54

		2623		90.57

		2622		90.61

		2621		90.64

		2620		90.67

		2619		90.7

		2618		90.72

		2617		90.75

		2616		90.77

		2615		90.79

		2614		90.8

		2613		90.82

		2612		90.83

		2611		90.84

		2610		90.85

		2609		90.87

		2608		90.88

		2607		90.9

		2606		90.91

		2605		90.93

		2604		90.96

		2603		90.98

		2602		91.01

		2601		91.04

		2600		91.07

		2599		91.1

		2598		91.14

		2597		91.17

		2596		91.21

		2595		91.25

		2594		91.28

		2593		91.32

		2592		91.35

		2591		91.38

		2590		91.41

		2589		91.43

		2588		91.45

		2587		91.48

		2586		91.49

		2585		91.51

		2584		91.52

		2583		91.54

		2582		91.55

		2581		91.56

		2580		91.57

		2579		91.58

		2578		91.59

		2577		91.6

		2576		91.61

		2575		91.62

		2574		91.62

		2573		91.63

		2572		91.63

		2571		91.64

		2570		91.64

		2569		91.64

		2568		91.64

		2567		91.64

		2566		91.64

		2565		91.64

		2564		91.64

		2563		91.64

		2562		91.64

		2561		91.65

		2560		91.66

		2559		91.67

		2558		91.69

		2557		91.71

		2556		91.74

		2555		91.77

		2554		91.8

		2553		91.83

		2552		91.87

		2551		91.91

		2550		91.95

		2549		91.99

		2548		92.04

		2547		92.08

		2546		92.12

		2545		92.16

		2544		92.19

		2543		92.22

		2542		92.25

		2541		92.28

		2540		92.3

		2539		92.31

		2538		92.33

		2537		92.34

		2536		92.35

		2535		92.37

		2534		92.38

		2533		92.41

		2532		92.43

		2531		92.46

		2530		92.5

		2529		92.55

		2528		92.6

		2527		92.66

		2526		92.72

		2525		92.78

		2524		92.85

		2523		92.91

		2522		92.97

		2521		93.03

		2520		93.09

		2519		93.14

		2518		93.19

		2517		93.23

		2516		93.26

		2515		93.3

		2514		93.33

		2513		93.36

		2512		93.39

		2511		93.43

		2510		93.47

		2509		93.5

		2508		93.55

		2507		93.59

		2506		93.64

		2505		93.69

		2504		93.74

		2503		93.78

		2502		93.83

		2501		93.88

		2500		93.92

		2499		93.96

		2498		93.99

		2497		94.02

		2496		94.05

		2495		94.07

		2494		94.09

		2493		94.11

		2492		94.13

		2491		94.14

		2490		94.16

		2489		94.18

		2488		94.2

		2487		94.23

		2486		94.26

		2485		94.29

		2484		94.33

		2483		94.36

		2482		94.4

		2481		94.44

		2480		94.48

		2479		94.52

		2478		94.56

		2477		94.59

		2476		94.62

		2475		94.65

		2474		94.68

		2473		94.7

		2472		94.72

		2471		94.73

		2470		94.75

		2469		94.76

		2468		94.78

		2467		94.79

		2466		94.8

		2465		94.82

		2464		94.84

		2463		94.86

		2462		94.88

		2461		94.9

		2460		94.93

		2459		94.95

		2458		94.98

		2457		95.01

		2456		95.03

		2455		95.06

		2454		95.08

		2453		95.11

		2452		95.13

		2451		95.15

		2450		95.17

		2449		95.18

		2448		95.2

		2447		95.21

		2446		95.23

		2445		95.24

		2444		95.26

		2443		95.27

		2442		95.29

		2441		95.31

		2440		95.33

		2439		95.35

		2438		95.38

		2437		95.4

		2436		95.43

		2435		95.46

		2434		95.49

		2433		95.51

		2432		95.53

		2431		95.56

		2430		95.58

		2429		95.6

		2428		95.61

		2427		95.63

		2426		95.64

		2425		95.65

		2424		95.66

		2423		95.67

		2422		95.68

		2421		95.7

		2420		95.71

		2419		95.72

		2418		95.73

		2417		95.74

		2416		95.76

		2415		95.77

		2414		95.79

		2413		95.8

		2412		95.82

		2411		95.84

		2410		95.85

		2409		95.87

		2408		95.89

		2407		95.91

		2406		95.92

		2405		95.94

		2404		95.95

		2403		95.97

		2402		95.98

		2401		95.99

		2400		96.01

		2399		96.02

		2398		96.03

		2397		96.04

		2396		96.05

		2395		96.06

		2394		96.08

		2393		96.09

		2392		96.1

		2391		96.11

		2390		96.13

		2389		96.15

		2388		96.16

		2387		96.18

		2386		96.2

		2385		96.22

		2384		96.24

		2383		96.25

		2382		96.27

		2381		96.28

		2380		96.3

		2379		96.31

		2378		96.31

		2377		96.32

		2376		96.32

		2375		96.33

		2374		96.33

		2373		96.34

		2372		96.34

		2371		96.35

		2370		96.35

		2369		96.36

		2368		96.36

		2367		96.37

		2366		96.37

		2365		96.38

		2364		96.38

		2363		96.39

		2362		96.39

		2361		96.39

		2360		96.39

		2359		96.4

		2358		96.4

		2357		96.41

		2356		96.41

		2355		96.41

		2354		96.41

		2353		96.42

		2352		96.42

		2351		96.42

		2350		96.42

		2349		96.42

		2348		96.42

		2347		96.42

		2346		96.42

		2345		96.42

		2344		96.42

		2343		96.42

		2342		96.42

		2341		96.42

		2340		96.43

		2339		96.44

		2338		96.44

		2337		96.45

		2336		96.45

		2335		96.45

		2334		96.45

		2333		96.45

		2332		96.44

		2331		96.43

		2330		96.42

		2329		96.41

		2328		96.4

		2327		96.39

		2326		96.38

		2325		96.37

		2324		96.37

		2323		96.37

		2322		96.38

		2321		96.39

		2320		96.41

		2319		96.42

		2318		96.44

		2317		96.46

		2316		96.48

		2315		96.5

		2314		96.52

		2313		96.54

		2312		96.56

		2311		96.58

		2310		96.6

		2309		96.61

		2308		96.63

		2307		96.64

		2306		96.65

		2305		96.66

		2304		96.66

		2303		96.66

		2302		96.67

		2301		96.66

		2300		96.66

		2299		96.66

		2298		96.65

		2297		96.65

		2296		96.64

		2295		96.64

		2294		96.63

		2293		96.62

		2292		96.62

		2291		96.61

		2290		96.61

		2289		96.6

		2288		96.6

		2287		96.6

		2286		96.61

		2285		96.61

		2284		96.62

		2283		96.63

		2282		96.64

		2281		96.65

		2280		96.66

		2279		96.67

		2278		96.69

		2277		96.7

		2276		96.72

		2275		96.73

		2274		96.75

		2273		96.76

		2272		96.77

		2271		96.78

		2270		96.79

		2269		96.8

		2268		96.81

		2267		96.82

		2266		96.83

		2265		96.83

		2264		96.84

		2263		96.84

		2262		96.85

		2261		96.86

		2260		96.87

		2259		96.88

		2258		96.89

		2257		96.91

		2256		96.93

		2255		96.95

		2254		96.97

		2253		96.99

		2252		97.01

		2251		97.03

		2250		97.04

		2249		97.06

		2248		97.07

		2247		97.08

		2246		97.09

		2245		97.1

		2244		97.11

		2243		97.12

		2242		97.13

		2241		97.14

		2240		97.16

		2239		97.17

		2238		97.19

		2237		97.2

		2236		97.22

		2235		97.24

		2234		97.25

		2233		97.27

		2232		97.28

		2231		97.3

		2230		97.31

		2229		97.32

		2228		97.33

		2227		97.33

		2226		97.34

		2225		97.34

		2224		97.35

		2223		97.35

		2222		97.36

		2221		97.36

		2220		97.36

		2219		97.36

		2218		97.36

		2217		97.36

		2216		97.36

		2215		97.36

		2214		97.36

		2213		97.36

		2212		97.37

		2211		97.37

		2210		97.37

		2209		97.38

		2208		97.39

		2207		97.39

		2206		97.4

		2205		97.41

		2204		97.41

		2203		97.41

		2202		97.41

		2201		97.41

		2200		97.41

		2199		97.4

		2198		97.39

		2197		97.39

		2196		97.38

		2195		97.37

		2194		97.37

		2193		97.37

		2192		97.37

		2191		97.37

		2190		97.38

		2189		97.39

		2188		97.4

		2187		97.41

		2186		97.42

		2185		97.44

		2184		97.45

		2183		97.47

		2182		97.48

		2181		97.49

		2180		97.49

		2179		97.5

		2178		97.5

		2177		97.49

		2176		97.48

		2175		97.47

		2174		97.45

		2173		97.44

		2172		97.42

		2171		97.4

		2170		97.38

		2169		97.37

		2168		97.37

		2167		97.38

		2166		97.4

		2165		97.44

		2164		97.48

		2163		97.53

		2162		97.59

		2161		97.65

		2160		97.72

		2159		97.78

		2158		97.83

		2157		97.88

		2156		97.91

		2155		97.93

		2154		97.94

		2153		97.94

		2152		97.93

		2151		97.92

		2150		97.91

		2149		97.89

		2148		97.88

		2147		97.87

		2146		97.86

		2145		97.86

		2144		97.86

		2143		97.86

		2142		97.86

		2141		97.86

		2140		97.87

		2139		97.88

		2138		97.88

		2137		97.89

		2136		97.89

		2135		97.9

		2134		97.9

		2133		97.89

		2132		97.88

		2131		97.87

		2130		97.86

		2129		97.85

		2128		97.83

		2127		97.81

		2126		97.8

		2125		97.78

		2124		97.76

		2123		97.75

		2122		97.73

		2121		97.72

		2120		97.71

		2119		97.69

		2118		97.68

		2117		97.67

		2116		97.67

		2115		97.66

		2114		97.66

		2113		97.66

		2112		97.66

		2111		97.66

		2110		97.66

		2109		97.66

		2108		97.67

		2107		97.67

		2106		97.67

		2105		97.67

		2104		97.68

		2103		97.68

		2102		97.68

		2101		97.68

		2100		97.68

		2099		97.69

		2098		97.69

		2097		97.7

		2096		97.7

		2095		97.71

		2094		97.71

		2093		97.71

		2092		97.71

		2091		97.71

		2090		97.71

		2089		97.71

		2088		97.7

		2087		97.69

		2086		97.68

		2085		97.68

		2084		97.67

		2083		97.66

		2082		97.65

		2081		97.65

		2080		97.65

		2079		97.65

		2078		97.65

		2077		97.65

		2076		97.66

		2075		97.67

		2074		97.68

		2073		97.69

		2072		97.7

		2071		97.71

		2070		97.72

		2069		97.73

		2068		97.74

		2067		97.75

		2066		97.76

		2065		97.76

		2064		97.77

		2063		97.77

		2062		97.77

		2061		97.77

		2060		97.77

		2059		97.76

		2058		97.75

		2057		97.75

		2056		97.74

		2055		97.74

		2054		97.73

		2053		97.73

		2052		97.73

		2051		97.73

		2050		97.73

		2049		97.74

		2048		97.75

		2047		97.76

		2046		97.78

		2045		97.79

		2044		97.8

		2043		97.81

		2042		97.82

		2041		97.83

		2040		97.84

		2039		97.85

		2038		97.86

		2037		97.87

		2036		97.88

		2035		97.89

		2034		97.9

		2033		97.91

		2032		97.92

		2031		97.93

		2030		97.93

		2029		97.93

		2028		97.93

		2027		97.93

		2026		97.92

		2025		97.91

		2024		97.9

		2023		97.89

		2022		97.88

		2021		97.87

		2020		97.87

		2019		97.87

		2018		97.87

		2017		97.88

		2016		97.89

		2015		97.9

		2014		97.92

		2013		97.94

		2012		97.96

		2011		97.98

		2010		98

		2009		98.02

		2008		98.03

		2007		98.04

		2006		98.04

		2005		98.04

		2004		98.03

		2003		98.01

		2002		98

		2001		97.98

		2000		97.96

		1999		97.94

		1998		97.92

		1997		97.9

		1996		97.88

		1995		97.86

		1994		97.85

		1993		97.84

		1992		97.83

		1991		97.81

		1990		97.8

		1989		97.78

		1988		97.76

		1987		97.75

		1986		97.74

		1985		97.73

		1984		97.72

		1983		97.72

		1982		97.73

		1981		97.74

		1980		97.76

		1979		97.79

		1978		97.83

		1977		97.87

		1976		97.91

		1975		97.95

		1974		97.98

		1973		98.01

		1972		98.03

		1971		98.05

		1970		98.06

		1969		98.06

		1968		98.06

		1967		98.06

		1966		98.06

		1965		98.06

		1964		98.05

		1963		98.05

		1962		98.04

		1961		98.04

		1960		98.03

		1959		98.01

		1958		98

		1957		97.99

		1956		97.97

		1955		97.95

		1954		97.94

		1953		97.92

		1952		97.9

		1951		97.89

		1950		97.88

		1949		97.87

		1948		97.87

		1947		97.87

		1946		97.87

		1945		97.87

		1944		97.87

		1943		97.87

		1942		97.87

		1941		97.87

		1940		97.87

		1939		97.86

		1938		97.86

		1937		97.85

		1936		97.84

		1935		97.83

		1934		97.82

		1933		97.81

		1932		97.8

		1931		97.79

		1930		97.78

		1929		97.77

		1928		97.76

		1927		97.75

		1926		97.74

		1925		97.73

		1924		97.72

		1923		97.71

		1922		97.69

		1921		97.68

		1920		97.67

		1919		97.67

		1918		97.66

		1917		97.66

		1916		97.65

		1915		97.65

		1914		97.64

		1913		97.64

		1912		97.64

		1911		97.64

		1910		97.63

		1909		97.63

		1908		97.62

		1907		97.61

		1906		97.6

		1905		97.58

		1904		97.57

		1903		97.55

		1902		97.54

		1901		97.52

		1900		97.51

		1899		97.5

		1898		97.49

		1897		97.48

		1896		97.48

		1895		97.48

		1894		97.47

		1893		97.47

		1892		97.47

		1891		97.48

		1890		97.48

		1889		97.47

		1888		97.47

		1887		97.47

		1886		97.46

		1885		97.45

		1884		97.44

		1883		97.43

		1882		97.42

		1881		97.41

		1880		97.4

		1879		97.38

		1878		97.37

		1877		97.36

		1876		97.35

		1875		97.33

		1874		97.32

		1873		97.31

		1872		97.3

		1871		97.29

		1870		97.28

		1869		97.27

		1868		97.26

		1867		97.25

		1866		97.24

		1865		97.23

		1864		97.22

		1863		97.2

		1862		97.19

		1861		97.17

		1860		97.16

		1859		97.14

		1858		97.13

		1857		97.11

		1856		97.09

		1855		97.08

		1854		97.06

		1853		97.04

		1852		97.03

		1851		97.01

		1850		97

		1849		96.98

		1848		96.97

		1847		96.96

		1846		96.95

		1845		96.93

		1844		96.92

		1843		96.91

		1842		96.9

		1841		96.89

		1840		96.87

		1839		96.86

		1838		96.86

		1837		96.85

		1836		96.84

		1835		96.83

		1834		96.82

		1833		96.81

		1832		96.79

		1831		96.78

		1830		96.76

		1829		96.74

		1828		96.72

		1827		96.69

		1826		96.67

		1825		96.64

		1824		96.61

		1823		96.58

		1822		96.55

		1821		96.53

		1820		96.5

		1819		96.48

		1818		96.46

		1817		96.44

		1816		96.42

		1815		96.41

		1814		96.39

		1813		96.38

		1812		96.37

		1811		96.36

		1810		96.35

		1809		96.34

		1808		96.33

		1807		96.32

		1806		96.3

		1805		96.29

		1804		96.27

		1803		96.25

		1802		96.23

		1801		96.21

		1800		96.18

		1799		96.14

		1798		96.11

		1797		96.06

		1796		96.02

		1795		95.97

		1794		95.92

		1793		95.86

		1792		95.81

		1791		95.75

		1790		95.7

		1789		95.66

		1788		95.62

		1787		95.59

		1786		95.57

		1785		95.57

		1784		95.57

		1783		95.58

		1782		95.61

		1781		95.64

		1780		95.69

		1779		95.73

		1778		95.78

		1777		95.83

		1776		95.88

		1775		95.93

		1774		95.98

		1773		96.03

		1772		96.07

		1771		96.11

		1770		96.14

		1769		96.17

		1768		96.2

		1767		96.23

		1766		96.26

		1765		96.28

		1764		96.31

		1763		96.33

		1762		96.35

		1761		96.37

		1760		96.38

		1759		96.4

		1758		96.41

		1757		96.42

		1756		96.42

		1755		96.42

		1754		96.42

		1753		96.42

		1752		96.41

		1751		96.39

		1750		96.37

		1749		96.34

		1748		96.31

		1747		96.27

		1746		96.22

		1745		96.17

		1744		96.1

		1743		96.03

		1742		95.94

		1741		95.85

		1740		95.74

		1739		95.61

		1738		95.48

		1737		95.33

		1736		95.16

		1735		94.96

		1734		94.75

		1733		94.51

		1732		94.23

		1731		93.92

		1730		93.57

		1729		93.18

		1728		92.73

		1727		92.21

		1726		91.61

		1725		90.92

		1724		90.12

		1723		89.21

		1722		88.2

		1721		87.07

		1720		85.82

		1719		84.46

		1718		82.98

		1717		81.4

		1716		79.74

		1715		78.01

		1714		76.2

		1713		74.32

		1712		72.39

		1711		70.4

		1710		68.39

		1709		66.34

		1708		64.29

		1707		62.25

		1706		60.25

		1705		58.33

		1704		56.54

		1703		54.89

		1702		53.41

		1701		52.13

		1700		51.05

		1699		50.22

		1698		49.61

		1697		49.24

		1696		49.06

		1695		49.06

		1694		49.21

		1693		49.5

		1692		49.9

		1691		50.43

		1690		51.06

		1689		51.79

		1688		52.63

		1687		53.6

		1686		54.69

		1685		55.94

		1684		57.35

		1683		58.91

		1682		60.61

		1681		62.43

		1680		64.36

		1679		66.36

		1678		68.4

		1677		70.45

		1676		72.49

		1675		74.45

		1674		76.32

		1673		78.08

		1672		79.7

		1671		81.2

		1670		82.56

		1669		83.79

		1668		84.88

		1667		85.85

		1666		86.71

		1665		87.47

		1664		88.14

		1663		88.75

		1662		89.28

		1661		89.77

		1660		90.2

		1659		90.58

		1658		90.93

		1657		91.25

		1656		91.54

		1655		91.81

		1654		92.06

		1653		92.29

		1652		92.5

		1651		92.69

		1650		92.87

		1649		93.04

		1648		93.2

		1647		93.35

		1646		93.5

		1645		93.64

		1644		93.77

		1643		93.9

		1642		94.03

		1641		94.15

		1640		94.27

		1639		94.38

		1638		94.49

		1637		94.6

		1636		94.71

		1635		94.81

		1634		94.9

		1633		94.99

		1632		95.08

		1631		95.17

		1630		95.25

		1629		95.33

		1628		95.41

		1627		95.49

		1626		95.56

		1625		95.63

		1624		95.7

		1623		95.77

		1622		95.84

		1621		95.91

		1620		95.97

		1619		96.04

		1618		96.1

		1617		96.16

		1616		96.23

		1615		96.28

		1614		96.34

		1613		96.4

		1612		96.45

		1611		96.5

		1610		96.54

		1609		96.59

		1608		96.63

		1607		96.67

		1606		96.7

		1605		96.73

		1604		96.76

		1603		96.79

		1602		96.81

		1601		96.83

		1600		96.85

		1599		96.87

		1598		96.89

		1597		96.9

		1596		96.92

		1595		96.94

		1594		96.96

		1593		96.98

		1592		97

		1591		97.02

		1590		97.04

		1589		97.06

		1588		97.08

		1587		97.1

		1586		97.11

		1585		97.13

		1584		97.15

		1583		97.16

		1582		97.17

		1581		97.18

		1580		97.19

		1579		97.2

		1578		97.2

		1577		97.21

		1576		97.21

		1575		97.21

		1574		97.21

		1573		97.21

		1572		97.21

		1571		97.21

		1570		97.21

		1569		97.2

		1568		97.2

		1567		97.2

		1566		97.2

		1565		97.2

		1564		97.21

		1563		97.21

		1562		97.22

		1561		97.22

		1560		97.23

		1559		97.24

		1558		97.24

		1557		97.25

		1556		97.26

		1555		97.26

		1554		97.26

		1553		97.27

		1552		97.27

		1551		97.27

		1550		97.27

		1549		97.27

		1548		97.28

		1547		97.28

		1546		97.28

		1545		97.29

		1544		97.29

		1543		97.3

		1542		97.3

		1541		97.31

		1540		97.32

		1539		97.32

		1538		97.33

		1537		97.33

		1536		97.33

		1535		97.33

		1534		97.33

		1533		97.32

		1532		97.32

		1531		97.31

		1530		97.3

		1529		97.29

		1528		97.28

		1527		97.27

		1526		97.25

		1525		97.24

		1524		97.23

		1523		97.22

		1522		97.2

		1521		97.19

		1520		97.17

		1519		97.16

		1518		97.15

		1517		97.13

		1516		97.12

		1515		97.1

		1514		97.09

		1513		97.08

		1512		97.07

		1511		97.06

		1510		97.06

		1509		97.05

		1508		97.04

		1507		97.04

		1506		97.03

		1505		97.02

		1504		97.01

		1503		97

		1502		96.99

		1501		96.98

		1500		96.96

		1499		96.94

		1498		96.92

		1497		96.9

		1496		96.87

		1495		96.84

		1494		96.81

		1493		96.78

		1492		96.74

		1491		96.7

		1490		96.65

		1489		96.58

		1488		96.51

		1487		96.41

		1486		96.28

		1485		96.11

		1484		95.86

		1483		95.51

		1482		95.01

		1481		94.33

		1480		93.49

		1479		92.49

		1478		91.38

		1477		90.17

		1476		88.9

		1475		87.6

		1474		86.31

		1473		85.1

		1472		84.05

		1471		83.24

		1470		82.67

		1469		82.32

		1468		82.15

		1467		82.11

		1466		82.2

		1465		82.4

		1464		82.72

		1463		83.14

		1462		83.6

		1461		84.08

		1460		84.54

		1459		85

		1458		85.46

		1457		85.93

		1456		86.4

		1455		86.84

		1454		87.25

		1453		87.59

		1452		87.86

		1451		88.05

		1450		88.17

		1449		88.21

		1448		88.19

		1447		88.09

		1446		87.92

		1445		87.69

		1444		87.41

		1443		87.06

		1442		86.65

		1441		86.18

		1440		85.66

		1439		85.1

		1438		84.49

		1437		83.85

		1436		83.21

		1435		82.59

		1434		82.01

		1433		81.5

		1432		81.09

		1431		80.8

		1430		80.64

		1429		80.63

		1428		80.77

		1427		81.05

		1426		81.44

		1425		81.91

		1424		82.42

		1423		82.94

		1422		83.41

		1421		83.8

		1420		84.07

		1419		84.23

		1418		84.25

		1417		84.15

		1416		83.95

		1415		83.68

		1414		83.38

		1413		83.11

		1412		82.91

		1411		82.84

		1410		82.91

		1409		83.15

		1408		83.55

		1407		84.11

		1406		84.8

		1405		85.6

		1404		86.47

		1403		87.38

		1402		88.27

		1401		89.14

		1400		89.94

		1399		90.66

		1398		91.3

		1397		91.85

		1396		92.32

		1395		92.72

		1394		93.05

		1393		93.32

		1392		93.55

		1391		93.73

		1390		93.87

		1389		93.98

		1388		94.05

		1387		94.09

		1386		94.11

		1385		94.1

		1384		94.06

		1383		93.99

		1382		93.9

		1381		93.79

		1380		93.67

		1379		93.54

		1378		93.41

		1377		93.29

		1376		93.17

		1375		93.06

		1374		92.97

		1373		92.89

		1372		92.82

		1371		92.76

		1370		92.7

		1369		92.63

		1368		92.53

		1367		92.41

		1366		92.27

		1365		92.09

		1364		91.88

		1363		91.65

		1362		91.4

		1361		91.13

		1360		90.85

		1359		90.57

		1358		90.31

		1357		90.07

		1356		89.85

		1355		89.67

		1354		89.53

		1353		89.44

		1352		89.39

		1351		89.4

		1350		89.47

		1349		89.6

		1348		89.79

		1347		90.03

		1346		90.3

		1345		90.6

		1344		90.91

		1343		91.19

		1342		91.44

		1341		91.62

		1340		91.72

		1339		91.72

		1338		91.63

		1337		91.43

		1336		91.16

		1335		90.81

		1334		90.43

		1333		90.04

		1332		89.67

		1331		89.35

		1330		89.11

		1329		88.96

		1328		88.9

		1327		88.93

		1326		89.02

		1325		89.14

		1324		89.27

		1323		89.36

		1322		89.37

		1321		89.26

		1320		89

		1319		88.57

		1318		87.95

		1317		87.15

		1316		86.2

		1315		85.12

		1314		83.94

		1313		82.73

		1312		81.52

		1311		80.37

		1310		79.33

		1309		78.44

		1308		77.72

		1307		77.19

		1306		76.84

		1305		76.65

		1304		76.59

		1303		76.63

		1302		76.74

		1301		76.88

		1300		77

		1299		77.08

		1298		77.07

		1297		76.95

		1296		76.72

		1295		76.38

		1294		75.96

		1293		75.49

		1292		75.02

		1291		74.57

		1290		74.19

		1289		73.9

		1288		73.77

		1287		73.84

		1286		74.14

		1285		74.67

		1284		75.43

		1283		76.39

		1282		77.5

		1281		78.73

		1280		80.02

		1279		81.32

		1278		82.6

		1277		83.79

		1276		84.85

		1275		85.73

		1274		86.42

		1273		86.89

		1272		87.13

		1271		87.15

		1270		86.97

		1269		86.62

		1268		86.14

		1267		85.57

		1266		84.96

		1265		84.37

		1264		83.85

		1263		83.48

		1262		83.3

		1261		83.34

		1260		83.61

		1259		84.08

		1258		84.73

		1257		85.51

		1256		86.38

		1255		87.3

		1254		88.2

		1253		89.04

		1252		89.77

		1251		90.35

		1250		90.76

		1249		90.97

		1248		90.96

		1247		90.72

		1246		90.26

		1245		89.61

		1244		88.8

		1243		87.86

		1242		86.84

		1241		85.8

		1240		84.81

		1239		83.95

		1238		83.3

		1237		82.91

		1236		82.8

		1235		82.99

		1234		83.43

		1233		84.09

		1232		84.91

		1231		85.84

		1230		86.81

		1229		87.75

		1228		88.61

		1227		89.34

		1226		89.88

		1225		90.21

		1224		90.34

		1223		90.25

		1222		89.98

		1221		89.53

		1220		88.95

		1219		88.26

		1218		87.5

		1217		86.72

		1216		85.98

		1215		85.33

		1214		84.83

		1213		84.53

		1212		84.45

		1211		84.58

		1210		84.91

		1209		85.43

		1208		86.1

		1207		86.89

		1206		87.74

		1205		88.6

		1204		89.41

		1203		90.1

		1202		90.61

		1201		90.93

		1200		91.02

		1199		90.88

		1198		90.55

		1197		90.05

		1196		89.42

		1195		88.72

		1194		88.01

		1193		87.35

		1192		86.81

		1191		86.45

		1190		86.33

		1189		86.47

		1188		86.84

		1187		87.4

		1186		88.11

		1185		88.92

		1184		89.78

		1183		90.66

		1182		91.51

		1181		92.28

		1180		92.96

		1179		93.53

		1178		93.99

		1177		94.36

		1176		94.65

		1175		94.9

		1174		95.1

		1173		95.27

		1172		95.42

		1171		95.55

		1170		95.66

		1169		95.76

		1168		95.85

		1167		95.93

		1166		96.01

		1165		96.07

		1164		96.13

		1163		96.19

		1162		96.24

		1161		96.28

		1160		96.32

		1159		96.36

		1158		96.4

		1157		96.43

		1156		96.46

		1155		96.49

		1154		96.52

		1153		96.54

		1152		96.56

		1151		96.58

		1150		96.6

		1149		96.62

		1148		96.63

		1147		96.65

		1146		96.66

		1145		96.67

		1144		96.68

		1143		96.69

		1142		96.69

		1141		96.7

		1140		96.69

		1139		96.68

		1138		96.66

		1137		96.63

		1136		96.59

		1135		96.52

		1134		96.44

		1133		96.34

		1132		96.21

		1131		96.08

		1130		95.93

		1129		95.77

		1128		95.63

		1127		95.49

		1126		95.38

		1125		95.29

		1124		95.24

		1123		95.22

		1122		95.24

		1121		95.29

		1120		95.37

		1119		95.46

		1118		95.57

		1117		95.67

		1116		95.76

		1115		95.85

		1114		95.92

		1113		95.98

		1112		96.02

		1111		96.04

		1110		96.05

		1109		96.06

		1108		96.05

		1107		96.03

		1106		95.99

		1105		95.93

		1104		95.82

		1103		95.65

		1102		95.42

		1101		95.11

		1100		94.75

		1099		94.33

		1098		93.89

		1097		93.43

		1096		92.98

		1095		92.57

		1094		92.22

		1093		91.97

		1092		91.85

		1091		91.84

		1090		91.95

		1089		92.14

		1088		92.41

		1087		92.71

		1086		93.03

		1085		93.36

		1084		93.66

		1083		93.92

		1082		94.14

		1081		94.3

		1080		94.41

		1079		94.48

		1078		94.52

		1077		94.54

		1076		94.55

		1075		94.54

		1074		94.51

		1073		94.49

		1072		94.45

		1071		94.41

		1070		94.37

		1069		94.32

		1068		94.27

		1067		94.22

		1066		94.17

		1065		94.12

		1064		94.08

		1063		94.05

		1062		94.01

		1061		93.98

		1060		93.94

		1059		93.91

		1058		93.88

		1057		93.85

		1056		93.83

		1055		93.82

		1054		93.81

		1053		93.8

		1052		93.81

		1051		93.82

		1050		93.83

		1049		93.84

		1048		93.85

		1047		93.86

		1046		93.86

		1045		93.85

		1044		93.84

		1043		93.81

		1042		93.78

		1041		93.75

		1040		93.73

		1039		93.72

		1038		93.72

		1037		93.74

		1036		93.77

		1035		93.81

		1034		93.87

		1033		93.94

		1032		94.03

		1031		94.11

		1030		94.19

		1029		94.26

		1028		94.32

		1027		94.36

		1026		94.39

		1025		94.42

		1024		94.43

		1023		94.43

		1022		94.42

		1021		94.4

		1020		94.38

		1019		94.36

		1018		94.34

		1017		94.32

		1016		94.29

		1015		94.27

		1014		94.24

		1013		94.2

		1012		94.17

		1011		94.13

		1010		94.08

		1009		94.02

		1008		93.96

		1007		93.89

		1006		93.83

		1005		93.76

		1004		93.7

		1003		93.64

		1002		93.59

		1001		93.56

		1000		93.53

		999		93.52

		998		93.53

		997		93.55

		996		93.56

		995		93.58

		994		93.58

		993		93.57

		992		93.55

		991		93.52

		990		93.47

		989		93.4

		988		93.33

		987		93.24

		986		93.15

		985		93.06

		984		92.98

		983		92.89

		982		92.79

		981		92.68

		980		92.55

		979		92.4

		978		92.22

		977		92.01

		976		91.76

		975		91.48

		974		91.15

		973		90.79

		972		90.4

		971		89.98

		970		89.54

		969		89.08

		968		88.6

		967		88.12

		966		87.63

		965		87.14

		964		86.64

		963		86.14

		962		85.65

		961		85.15

		960		84.65

		959		84.16

		958		83.66

		957		83.15

		956		82.64

		955		82.12

		954		81.58

		953		81.04

		952		80.47

		951		79.89

		950		79.28

		949		78.66

		948		78.02

		947		77.39

		946		76.76

		945		76.16

		944		75.59

		943		75.08

		942		74.63

		941		74.28

		940		74.02

		939		73.88

		938		73.85

		937		73.94

		936		74.15

		935		74.47

		934		74.9

		933		75.43

		932		76.04

		931		76.72

		930		77.45

		929		78.21

		928		79

		927		79.8

		926		80.59

		925		81.35

		924		82.09

		923		82.78

		922		83.41

		921		83.98

		920		84.48

		919		84.9

		918		85.25

		917		85.52

		916		85.72

		915		85.86

		914		85.96

		913		86.02

		912		86.06

		911		86.11

		910		86.17

		909		86.27

		908		86.39

		907		86.56

		906		86.76

		905		86.99

		904		87.24

		903		87.49

		902		87.72

		901		87.91

		900		88.07

		899		88.17

		898		88.22

		897		88.21

		896		88.15

		895		88.07

		894		87.96

		893		87.86

		892		87.78

		891		87.73

		890		87.72

		889		87.76

		888		87.86

		887		88.02

		886		88.24

		885		88.51

		884		88.81

		883		89.13

		882		89.45

		881		89.78

		880		90.1

		879		90.41

		878		90.7

		877		90.96

		876		91.21

		875		91.43

		874		91.64

		873		91.83

		872		92.01

		871		92.18

		870		92.34

		869		92.5

		868		92.64

		867		92.78

		866		92.92

		865		93.05

		864		93.18

		863		93.31

		862		93.44

		861		93.57

		860		93.7

		859		93.84

		858		93.98

		857		94.12

		856		94.26

		855		94.41

		854		94.55

		853		94.68

		852		94.81

		851		94.94

		850		95.06

		849		95.17

		848		95.27

		847		95.36

		846		95.45

		845		95.53

		844		95.61

		843		95.68

		842		95.75

		841		95.82

		840		95.88

		839		95.93

		838		95.99

		837		96.04

		836		96.08

		835		96.12

		834		96.16

		833		96.19

		832		96.22

		831		96.24

		830		96.25

		829		96.26

		828		96.24

		827		96.21

		826		96.15

		825		96.05

		824		95.92

		823		95.74

		822		95.54

		821		95.32

		820		95.09

		819		94.88

		818		94.68

		817		94.52

		816		94.42

		815		94.39

		814		94.45

		813		94.59

		812		94.8

		811		95.06

		810		95.35

		809		95.65

		808		95.95

		807		96.24

		806		96.5

		805		96.73

		804		96.92

		803		97.06

		802		97.16

		801		97.24

		800		97.3

		799		97.34

		798		97.38

		797		97.41

		796		97.42

		795		97.43

		794		97.43

		793		97.42

		792		97.39

		791		97.34

		790		97.27

		789		97.18

		788		97.08

		787		96.97

		786		96.87

		785		96.77

		784		96.69

		783		96.62

		782		96.58

		781		96.58

		780		96.62

		779		96.69

		778		96.78

		777		96.89

		776		97

		775		97.12

		774		97.23

		773		97.33

		772		97.41

		771		97.48

		770		97.52

		769		97.55

		768		97.55

		767		97.52

		766		97.48

		765		97.4

		764		97.27

		763		97.1

		762		96.88

		761		96.61

		760		96.31

		759		95.99

		758		95.67

		757		95.36

		756		95.09

		755		94.86

		754		94.72

		753		94.67

		752		94.72

		751		94.87

		750		95.08

		749		95.34

		748		95.62

		747		95.88

		746		96.12

		745		96.31

		744		96.45

		743		96.5

		742		96.46

		741		96.31

		740		96.04

		739		95.65

		738		95.11

		737		94.42

		736		93.57

		735		92.58

		734		91.46

		733		90.24

		732		88.95

		731		87.59

		730		86.22

		729		84.88

		728		83.65

		727		82.6

		726		81.8

		725		81.26

		724		80.98

		723		80.95

		722		81.17

		721		81.64

		720		82.38

		719		83.36

		718		84.53

		717		85.8

		716		87.09

		715		88.37

		714		89.58

		713		90.7

		712		91.73

		711		92.62

		710		93.36

		709		93.95

		708		94.37

		707		94.66

		706		94.83

		705		94.9

		704		94.89

		703		94.8

		702		94.64

		701		94.4

		700		94.07

		699		93.65

		698		93.16

		697		92.58

		696		91.94

		695		91.24

		694		90.51

		693		89.78

		692		89.08

		691		88.43

		690		87.86

		689		87.4

		688		87.06

		687		86.86

		686		86.78

		685		86.83

		684		87

		683		87.25

		682		87.56

		681		87.93

		680		88.31

		679		88.7

		678		89.07

		677		89.43

		676		89.76

		675		90.07

		674		90.36

		673		90.63

		672		90.89

		671		91.14

		670		91.4

		669		91.66

		668		91.93

		667		92.2

		666		92.49

		665		92.78

		664		93.07

		663		93.38

		662		93.68

		661		93.98

		660		94.27

		659		94.56

		658		94.83

		657		95.08

		656		95.33

		655		95.55

		654		95.75

		653		95.93

		652		96.1

		651		96.24

		650		96.36

		649		96.47

		648		96.56

		647		96.63

		646		96.69

		645		96.73

		644		96.76

		643		96.79

		642		96.81

		641		96.82

		640		96.83

		639		96.85

		638		96.86

		637		96.88

		636		96.92

		635		96.95

		634		97

		633		97.05

		632		97.11

		631		97.17

		630		97.23

		629		97.29

		628		97.36

		627		97.42

		626		97.47

		625		97.53

		624		97.57

		623		97.62

		622		97.65

		621		97.69

		620		97.72

		619		97.75

		618		97.77

		617		97.8

		616		97.81

		615		97.83

		614		97.85

		613		97.87

		612		97.88

		611		97.9

		610		97.91

		609		97.92

		608		97.94

		607		97.95

		606		97.97

		605		97.98

		604		98

		603		98.01

		602		98.02

		601		98.03

		600		98.04

		599		98.05

		598		98.06

		597		98.06

		596		98.06

		595		98.06

		594		98.06

		593		98.06

		592		98.05

		591		98.05

		590		98.04

		589		98.03

		588		98.01

		587		97.99

		586		97.97

		585		97.94

		584		97.9

		583		97.85

		582		97.8

		581		97.73

		580		97.65

		579		97.56

		578		97.45

		577		97.32

		576		97.19

		575		97.03

		574		96.86

		573		96.67

		572		96.46

		571		96.23

		570		95.98

		569		95.71

		568		95.42

		567		95.1

		566		94.76

		565		94.39

		564		94

		563		93.58

		562		93.13

		561		92.66

		560		92.16

		559		91.65

		558		91.12

		557		90.59

		556		90.06

		555		89.55

		554		89.07

		553		88.64

		552		88.27

		551		87.98

		550		87.79

		549		87.7

		548		87.73

		547		87.88

		546		88.16

		545		88.54

		544		89.02

		543		89.58

		542		90.21

		541		90.88

		540		91.56

		539		92.25

		538		92.92

		537		93.55

		536		94.13

		535		94.65

		534		95.12

		533		95.53

		532		95.88

		531		96.18

		530		96.44

		529		96.66

		528		96.84

		527		96.99

		526		97.12

		525		97.23

		524		97.33

		523		97.43

		522		97.5

		521		97.57

		520		97.64

		519		97.69

		518		97.73

		517		97.75

		516		97.76

		515		97.74

		514		97.69

		513		97.6

		512		97.46

		511		97.26

		510		96.99

		509		96.64

		508		96.23

		507		95.75

		506		95.23

		505		94.68

		504		94.14

		503		93.62

		502		93.16

		501		92.79

		500		92.55

		499		92.44

		498		92.47

		497		92.63

		496		92.91

		495		93.27

		494		93.7

		493		94.16

		492		94.63

		491		95.08

		490		95.49

		489		95.85

		488		96.15

		487		96.39

		486		96.58

		485		96.73

		484		96.85

		483		96.95

		482		97.02

		481		97.09

		480		97.15

		479		97.21

		478		97.27

		477		97.33

		476		97.39

		475		97.45

		474		97.51

		473		97.56

		472		97.61

		471		97.66

		470		97.7

		469		97.73

		468		97.76

		467		97.77

		466		97.78

		465		97.79

		464		97.79

		463		97.79

		462		97.77

		461		97.75

		460		97.72

		459		97.69

		458		97.65

		457		97.6

		456		97.54

		455		97.47

		454		97.38

		453		97.28

		452		97.15

		451		97.01

		450		96.83

		449		96.61

		448		96.33

		447		95.99

		446		95.57

		445		95.08

		444		94.52

		443		93.92

		442		93.29

		441		92.67

		440		92.08

		439		91.56

		438		91.14

		437		90.86

		436		90.75

		435		90.81

		434		91.04

		433		91.42

		432		91.91

		431		92.49

		430		93.12

		429		93.76

		428		94.38

		427		94.95

		426		95.45

		425		95.85

		424		96.14

		423		96.33

		422		96.42

		421		96.45

		420		96.42

		419		96.36

		418		96.29

		417		96.23

		416		96.18

		415		96.17

		414		96.21

		413		96.29

		412		96.44

		411		96.62

		410		96.84

		409		97.07

		408		97.3

		407		97.51

		406		97.69

		405		97.83

		404		97.94

		403		98.02

		402		98.06

		401		98.06

		400		98.06
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		cm-1		%T

		4000		96.65

		3999		96.65

		3998		96.65

		3997		96.65

		3996		96.65

		3995		96.65

		3994		96.65

		3993		96.65

		3992		96.65

		3991		96.65

		3990		96.65

		3989		96.65

		3988		96.64

		3987		96.64

		3986		96.64

		3985		96.64

		3984		96.63

		3983		96.63

		3982		96.63

		3981		96.63

		3980		96.63

		3979		96.63

		3978		96.63

		3977		96.63

		3976		96.63

		3975		96.63

		3974		96.63

		3973		96.63

		3972		96.64

		3971		96.64

		3970		96.64

		3969		96.64

		3968		96.64

		3967		96.64

		3966		96.64

		3965		96.64

		3964		96.64

		3963		96.64

		3962		96.64

		3961		96.64

		3960		96.64

		3959		96.64

		3958		96.64

		3957		96.64

		3956		96.64

		3955		96.64

		3954		96.64

		3953		96.63

		3952		96.63

		3951		96.63

		3950		96.63

		3949		96.62

		3948		96.62

		3947		96.62

		3946		96.62

		3945		96.62

		3944		96.62

		3943		96.62

		3942		96.62

		3941		96.62

		3940		96.63

		3939		96.63

		3938		96.63

		3937		96.63

		3936		96.63

		3935		96.63

		3934		96.63

		3933		96.63

		3932		96.63

		3931		96.63

		3930		96.63

		3929		96.63

		3928		96.63

		3927		96.63

		3926		96.63

		3925		96.62

		3924		96.62

		3923		96.62

		3922		96.61

		3921		96.61

		3920		96.6

		3919		96.6

		3918		96.6

		3917		96.6

		3916		96.59

		3915		96.59

		3914		96.59

		3913		96.59

		3912		96.59

		3911		96.59

		3910		96.59

		3909		96.59

		3908		96.59

		3907		96.58

		3906		96.58

		3905		96.58

		3904		96.58

		3903		96.57

		3902		96.57

		3901		96.57

		3900		96.57

		3899		96.58

		3898		96.58

		3897		96.58

		3896		96.58

		3895		96.58

		3894		96.58

		3893		96.58

		3892		96.58

		3891		96.58

		3890		96.58

		3889		96.58

		3888		96.58

		3887		96.58

		3886		96.58

		3885		96.57

		3884		96.57

		3883		96.57

		3882		96.57

		3881		96.57

		3880		96.57

		3879		96.57

		3878		96.57

		3877		96.57

		3876		96.57

		3875		96.56

		3874		96.56

		3873		96.56

		3872		96.56

		3871		96.56

		3870		96.56

		3869		96.56

		3868		96.56

		3867		96.55

		3866		96.55

		3865		96.55

		3864		96.56

		3863		96.56

		3862		96.56

		3861		96.56

		3860		96.56

		3859		96.57

		3858		96.57

		3857		96.57

		3856		96.57

		3855		96.57

		3854		96.57

		3853		96.57

		3852		96.57

		3851		96.57

		3850		96.57

		3849		96.57

		3848		96.56

		3847		96.56

		3846		96.56

		3845		96.55

		3844		96.55

		3843		96.54

		3842		96.54

		3841		96.54

		3840		96.53

		3839		96.53

		3838		96.53

		3837		96.53

		3836		96.53

		3835		96.53

		3834		96.54

		3833		96.54

		3832		96.54

		3831		96.54

		3830		96.54

		3829		96.55

		3828		96.55

		3827		96.55

		3826		96.54

		3825		96.54

		3824		96.54

		3823		96.54

		3822		96.54

		3821		96.55

		3820		96.55

		3819		96.55

		3818		96.55

		3817		96.56

		3816		96.56

		3815		96.56

		3814		96.57

		3813		96.57

		3812		96.57

		3811		96.57

		3810		96.56

		3809		96.56

		3808		96.56

		3807		96.55

		3806		96.55

		3805		96.55

		3804		96.54

		3803		96.55

		3802		96.55

		3801		96.55

		3800		96.55

		3799		96.56

		3798		96.56

		3797		96.57

		3796		96.58

		3795		96.58

		3794		96.59

		3793		96.59

		3792		96.6

		3791		96.6

		3790		96.6

		3789		96.6

		3788		96.61

		3787		96.61

		3786		96.61

		3785		96.61

		3784		96.61

		3783		96.61

		3782		96.61

		3781		96.61

		3780		96.62

		3779		96.62

		3778		96.62

		3777		96.62

		3776		96.62

		3775		96.61

		3774		96.61

		3773		96.61

		3772		96.61

		3771		96.61

		3770		96.61

		3769		96.6

		3768		96.6

		3767		96.6

		3766		96.6

		3765		96.59

		3764		96.59

		3763		96.59

		3762		96.58

		3761		96.58

		3760		96.58

		3759		96.57

		3758		96.56

		3757		96.55

		3756		96.54

		3755		96.53

		3754		96.52

		3753		96.51

		3752		96.5

		3751		96.49

		3750		96.49

		3749		96.49

		3748		96.49

		3747		96.49

		3746		96.49

		3745		96.5

		3744		96.5

		3743		96.51

		3742		96.51

		3741		96.51

		3740		96.52

		3739		96.52

		3738		96.52

		3737		96.52

		3736		96.53

		3735		96.53

		3734		96.53

		3733		96.54

		3732		96.54

		3731		96.54

		3730		96.55

		3729		96.55

		3728		96.55

		3727		96.55

		3726		96.55

		3725		96.55

		3724		96.55

		3723		96.55

		3722		96.54

		3721		96.54

		3720		96.53

		3719		96.52

		3718		96.51

		3717		96.5

		3716		96.49

		3715		96.48

		3714		96.47

		3713		96.46

		3712		96.45

		3711		96.44

		3710		96.44

		3709		96.43

		3708		96.42

		3707		96.42

		3706		96.41

		3705		96.4

		3704		96.4

		3703		96.39

		3702		96.37

		3701		96.36

		3700		96.35

		3699		96.33

		3698		96.32

		3697		96.3

		3696		96.28

		3695		96.27

		3694		96.26

		3693		96.24

		3692		96.23

		3691		96.22

		3690		96.21

		3689		96.2

		3688		96.19

		3687		96.18

		3686		96.17

		3685		96.16

		3684		96.14

		3683		96.13

		3682		96.12

		3681		96.11

		3680		96.1

		3679		96.08

		3678		96.07

		3677		96.06

		3676		96.05

		3675		96.05

		3674		96.04

		3673		96.04

		3672		96.04

		3671		96.04

		3670		96.04

		3669		96.05

		3668		96.05

		3667		96.06

		3666		96.06

		3665		96.06

		3664		96.07

		3663		96.07

		3662		96.08

		3661		96.09

		3660		96.09

		3659		96.1

		3658		96.11

		3657		96.11

		3656		96.12

		3655		96.13

		3654		96.14

		3653		96.16

		3652		96.17

		3651		96.19

		3650		96.2

		3649		96.22

		3648		96.24

		3647		96.26

		3646		96.28

		3645		96.29

		3644		96.31

		3643		96.33

		3642		96.35

		3641		96.37

		3640		96.38

		3639		96.39

		3638		96.41

		3637		96.42

		3636		96.43

		3635		96.43

		3634		96.44

		3633		96.45

		3632		96.46

		3631		96.46

		3630		96.47

		3629		96.48

		3628		96.49

		3627		96.5

		3626		96.5

		3625		96.51

		3624		96.52

		3623		96.52

		3622		96.53

		3621		96.53

		3620		96.53

		3619		96.53

		3618		96.52

		3617		96.52

		3616		96.51

		3615		96.5

		3614		96.5

		3613		96.49

		3612		96.49

		3611		96.48

		3610		96.48

		3609		96.48

		3608		96.48

		3607		96.49

		3606		96.49

		3605		96.5

		3604		96.51

		3603		96.52

		3602		96.53

		3601		96.54

		3600		96.55

		3599		96.56

		3598		96.57

		3597		96.57

		3596		96.58

		3595		96.59

		3594		96.6

		3593		96.6

		3592		96.61

		3591		96.61

		3590		96.62

		3589		96.62

		3588		96.63

		3587		96.63

		3586		96.63

		3585		96.64

		3584		96.64

		3583		96.64

		3582		96.65

		3581		96.65

		3580		96.65

		3579		96.65

		3578		96.65

		3577		96.65

		3576		96.65

		3575		96.65

		3574		96.65

		3573		96.65

		3572		96.65

		3571		96.65

		3570		96.65

		3569		96.65

		3568		96.65

		3567		96.64

		3566		96.64

		3565		96.64

		3564		96.64

		3563		96.64

		3562		96.64

		3561		96.64

		3560		96.65

		3559		96.65

		3558		96.65

		3557		96.65

		3556		96.65

		3555		96.65

		3554		96.65

		3553		96.65

		3552		96.64

		3551		96.64

		3550		96.64

		3549		96.64

		3548		96.64

		3547		96.64

		3546		96.64

		3545		96.64

		3544		96.64

		3543		96.64

		3542		96.64

		3541		96.64

		3540		96.64

		3539		96.64

		3538		96.64

		3537		96.65

		3536		96.65

		3535		96.65

		3534		96.64

		3533		96.64

		3532		96.64

		3531		96.64

		3530		96.64

		3529		96.64

		3528		96.64

		3527		96.64

		3526		96.64

		3525		96.65

		3524		96.65

		3523		96.65

		3522		96.65

		3521		96.65

		3520		96.65

		3519		96.65

		3518		96.65

		3517		96.65

		3516		96.65

		3515		96.65

		3514		96.65

		3513		96.65

		3512		96.65

		3511		96.65

		3510		96.65

		3509		96.64

		3508		96.64

		3507		96.64

		3506		96.64

		3505		96.64

		3504		96.64

		3503		96.64

		3502		96.64

		3501		96.64

		3500		96.64

		3499		96.64

		3498		96.64

		3497		96.65

		3496		96.65

		3495		96.65

		3494		96.65

		3493		96.65

		3492		96.65

		3491		96.65

		3490		96.65

		3489		96.65

		3488		96.65

		3487		96.65

		3486		96.65

		3485		96.65

		3484		96.65

		3483		96.65

		3482		96.65

		3481		96.65

		3480		96.64

		3479		96.64

		3478		96.64

		3477		96.64

		3476		96.64

		3475		96.64

		3474		96.64

		3473		96.64

		3472		96.64

		3471		96.64

		3470		96.64

		3469		96.64

		3468		96.64

		3467		96.64

		3466		96.64

		3465		96.64

		3464		96.64

		3463		96.64

		3462		96.64

		3461		96.63

		3460		96.63

		3459		96.63

		3458		96.63

		3457		96.62

		3456		96.62

		3455		96.62

		3454		96.62

		3453		96.62

		3452		96.61

		3451		96.61

		3450		96.61

		3449		96.61

		3448		96.61

		3447		96.6

		3446		96.6

		3445		96.6

		3444		96.6

		3443		96.6

		3442		96.6

		3441		96.6

		3440		96.6

		3439		96.6

		3438		96.59

		3437		96.59

		3436		96.59

		3435		96.58

		3434		96.58

		3433		96.57

		3432		96.57

		3431		96.56

		3430		96.55

		3429		96.54

		3428		96.53

		3427		96.52

		3426		96.51

		3425		96.5

		3424		96.49

		3423		96.49

		3422		96.48

		3421		96.48

		3420		96.47

		3419		96.47

		3418		96.47

		3417		96.46

		3416		96.46

		3415		96.46

		3414		96.46

		3413		96.46

		3412		96.46

		3411		96.45

		3410		96.45

		3409		96.45

		3408		96.45

		3407		96.45

		3406		96.45

		3405		96.45

		3404		96.45

		3403		96.45

		3402		96.46

		3401		96.46

		3400		96.46

		3399		96.46

		3398		96.45

		3397		96.45

		3396		96.45

		3395		96.44

		3394		96.43

		3393		96.42

		3392		96.41

		3391		96.39

		3390		96.38

		3389		96.37

		3388		96.35

		3387		96.34

		3386		96.33

		3385		96.33

		3384		96.32

		3383		96.32

		3382		96.31

		3381		96.31

		3380		96.32

		3379		96.32

		3378		96.33

		3377		96.34

		3376		96.34

		3375		96.35

		3374		96.36

		3373		96.36

		3372		96.37

		3371		96.37

		3370		96.38

		3369		96.37

		3368		96.37

		3367		96.37

		3366		96.36

		3365		96.35

		3364		96.34

		3363		96.33

		3362		96.32

		3361		96.31

		3360		96.3

		3359		96.29

		3358		96.29

		3357		96.28

		3356		96.28

		3355		96.28

		3354		96.28

		3353		96.28

		3352		96.28

		3351		96.28

		3350		96.28

		3349		96.27

		3348		96.27

		3347		96.27

		3346		96.26

		3345		96.25

		3344		96.25

		3343		96.24

		3342		96.23

		3341		96.23

		3340		96.22

		3339		96.21

		3338		96.21

		3337		96.2

		3336		96.2

		3335		96.19

		3334		96.18

		3333		96.18

		3332		96.17

		3331		96.16

		3330		96.16

		3329		96.15

		3328		96.15

		3327		96.14

		3326		96.14

		3325		96.14

		3324		96.13

		3323		96.13

		3322		96.12

		3321		96.12

		3320		96.12

		3319		96.11

		3318		96.11

		3317		96.11

		3316		96.11

		3315		96.11

		3314		96.11

		3313		96.11

		3312		96.11

		3311		96.11

		3310		96.11

		3309		96.11

		3308		96.11

		3307		96.11

		3306		96.11

		3305		96.1

		3304		96.1

		3303		96.09

		3302		96.08

		3301		96.07

		3300		96.07

		3299		96.06

		3298		96.05

		3297		96.04

		3296		96.03

		3295		96.02

		3294		96.02

		3293		96.01

		3292		96

		3291		95.99

		3290		95.98

		3289		95.96

		3288		95.95

		3287		95.94

		3286		95.94

		3285		95.93

		3284		95.92

		3283		95.91

		3282		95.9

		3281		95.89

		3280		95.89

		3279		95.88

		3278		95.87

		3277		95.86

		3276		95.85

		3275		95.85

		3274		95.84

		3273		95.83

		3272		95.82

		3271		95.81

		3270		95.79

		3269		95.78

		3268		95.77

		3267		95.76

		3266		95.75

		3265		95.73

		3264		95.72

		3263		95.71

		3262		95.7

		3261		95.69

		3260		95.68

		3259		95.67

		3258		95.66

		3257		95.64

		3256		95.63

		3255		95.62

		3254		95.6

		3253		95.59

		3252		95.58

		3251		95.56

		3250		95.55

		3249		95.53

		3248		95.52

		3247		95.5

		3246		95.49

		3245		95.47

		3244		95.46

		3243		95.44

		3242		95.43

		3241		95.41

		3240		95.39

		3239		95.38

		3238		95.36

		3237		95.35

		3236		95.33

		3235		95.32

		3234		95.3

		3233		95.28

		3232		95.27

		3231		95.25

		3230		95.23

		3229		95.22

		3228		95.2

		3227		95.18

		3226		95.17

		3225		95.15

		3224		95.13

		3223		95.12

		3222		95.1

		3221		95.08

		3220		95.07

		3219		95.05

		3218		95.03

		3217		95.02

		3216		95

		3215		94.98

		3214		94.97

		3213		94.95

		3212		94.93

		3211		94.91

		3210		94.9

		3209		94.88

		3208		94.86

		3207		94.84

		3206		94.82

		3205		94.81

		3204		94.79

		3203		94.77

		3202		94.75

		3201		94.73

		3200		94.71

		3199		94.7

		3198		94.68

		3197		94.66

		3196		94.65

		3195		94.63

		3194		94.62

		3193		94.6

		3192		94.58

		3191		94.57

		3190		94.55

		3189		94.53

		3188		94.52

		3187		94.5

		3186		94.48

		3185		94.46

		3184		94.45

		3183		94.43

		3182		94.42

		3181		94.4

		3180		94.39

		3179		94.37

		3178		94.36

		3177		94.34

		3176		94.33

		3175		94.31

		3174		94.3

		3173		94.28

		3172		94.26

		3171		94.24

		3170		94.23

		3169		94.21

		3168		94.19

		3167		94.17

		3166		94.15

		3165		94.13

		3164		94.11

		3163		94.09

		3162		94.07

		3161		94.05

		3160		94.03

		3159		94.01

		3158		93.99

		3157		93.97

		3156		93.94

		3155		93.92

		3154		93.9

		3153		93.88

		3152		93.85

		3151		93.83

		3150		93.8

		3149		93.78

		3148		93.75

		3147		93.72

		3146		93.7

		3145		93.67

		3144		93.64

		3143		93.61

		3142		93.58

		3141		93.55

		3140		93.52

		3139		93.49

		3138		93.46

		3137		93.43

		3136		93.4

		3135		93.37

		3134		93.34

		3133		93.31

		3132		93.27

		3131		93.24

		3130		93.21

		3129		93.18

		3128		93.15

		3127		93.11

		3126		93.08

		3125		93.05

		3124		93.02

		3123		92.99

		3122		92.95

		3121		92.92

		3120		92.89

		3119		92.86

		3118		92.82

		3117		92.79

		3116		92.76

		3115		92.72

		3114		92.69

		3113		92.65

		3112		92.62

		3111		92.58

		3110		92.55

		3109		92.52

		3108		92.48

		3107		92.45

		3106		92.42

		3105		92.39

		3104		92.35

		3103		92.32

		3102		92.29

		3101		92.26

		3100		92.23

		3099		92.21

		3098		92.18

		3097		92.15

		3096		92.12

		3095		92.1

		3094		92.07

		3093		92.05

		3092		92.02

		3091		92

		3090		91.98

		3089		91.96

		3088		91.93

		3087		91.91

		3086		91.89

		3085		91.87

		3084		91.85

		3083		91.83

		3082		91.81

		3081		91.79

		3080		91.76

		3079		91.74

		3078		91.72

		3077		91.7

		3076		91.67

		3075		91.65

		3074		91.63

		3073		91.6

		3072		91.58

		3071		91.56

		3070		91.53

		3069		91.5

		3068		91.48

		3067		91.45

		3066		91.42

		3065		91.4

		3064		91.37

		3063		91.34

		3062		91.31

		3061		91.28

		3060		91.25

		3059		91.22

		3058		91.18

		3057		91.15

		3056		91.11

		3055		91.08

		3054		91.04

		3053		91

		3052		90.96

		3051		90.92

		3050		90.88

		3049		90.83

		3048		90.79

		3047		90.74

		3046		90.69

		3045		90.64

		3044		90.59

		3043		90.54

		3042		90.48

		3041		90.43

		3040		90.37

		3039		90.31

		3038		90.25

		3037		90.19

		3036		90.13

		3035		90.07

		3034		90.01

		3033		89.94

		3032		89.88

		3031		89.82

		3030		89.76

		3029		89.69

		3028		89.63

		3027		89.57

		3026		89.51

		3025		89.45

		3024		89.39

		3023		89.34

		3022		89.28

		3021		89.22

		3020		89.17

		3019		89.11

		3018		89.06

		3017		89.01

		3016		88.96

		3015		88.91

		3014		88.86

		3013		88.81

		3012		88.76

		3011		88.72

		3010		88.68

		3009		88.63

		3008		88.59

		3007		88.56

		3006		88.52

		3005		88.49

		3004		88.45

		3003		88.42

		3002		88.39

		3001		88.36

		3000		88.33

		2999		88.29

		2998		88.26

		2997		88.22

		2996		88.18

		2995		88.14

		2994		88.1

		2993		88.05

		2992		88

		2991		87.95

		2990		87.9

		2989		87.85

		2988		87.8

		2987		87.75

		2986		87.7

		2985		87.65

		2984		87.59

		2983		87.53

		2982		87.47

		2981		87.39

		2980		87.31

		2979		87.2

		2978		87.07

		2977		86.91

		2976		86.71

		2975		86.45

		2974		86.14

		2973		85.76

		2972		85.31

		2971		84.81

		2970		84.25

		2969		83.66

		2968		83.03

		2967		82.39

		2966		81.74

		2965		81.1

		2964		80.49

		2963		79.91

		2962		79.38

		2961		78.9

		2960		78.47

		2959		78.12

		2958		77.82

		2957		77.6

		2956		77.47

		2955		77.41

		2954		77.44

		2953		77.56

		2952		77.73

		2951		77.95

		2950		78.19

		2949		78.43

		2948		78.63

		2947		78.78

		2946		78.85

		2945		78.85

		2944		78.75

		2943		78.55

		2942		78.27

		2941		77.91

		2940		77.5

		2939		77.04

		2938		76.56

		2937		76.06

		2936		75.56

		2935		75.06

		2934		74.54

		2933		73.99

		2932		73.4

		2931		72.75

		2930		72.02

		2929		71.17

		2928		70.18

		2927		69.04

		2926		67.74

		2925		66.27

		2924		64.66

		2923		62.91

		2922		61.1

		2921		59.26

		2920		57.48

		2919		55.83

		2918		54.39

		2917		53.21

		2916		52.36

		2915		51.88

		2914		51.79

		2913		52.08

		2912		52.74

		2911		53.71

		2910		54.93

		2909		56.33

		2908		57.84

		2907		59.4

		2906		60.95

		2905		62.44

		2904		63.84

		2903		65.13

		2902		66.3

		2901		67.34

		2900		68.28

		2899		69.12

		2898		69.88

		2897		70.58

		2896		71.22

		2895		71.83

		2894		72.41

		2893		72.97

		2892		73.51

		2891		74.05

		2890		74.57

		2889		75.1

		2888		75.61

		2887		76.12

		2886		76.6

		2885		77.06

		2884		77.48

		2883		77.85

		2882		78.16

		2881		78.4

		2880		78.57

		2879		78.67

		2878		78.71

		2877		78.69

		2876		78.63

		2875		78.55

		2874		78.46

		2873		78.38

		2872		78.32

		2871		78.3

		2870		78.3

		2869		78.33

		2868		78.36

		2867		78.37

		2866		78.35

		2865		78.25

		2864		78.07

		2863		77.76

		2862		77.29

		2861		76.64

		2860		75.77

		2859		74.68

		2858		73.37

		2857		71.86

		2856		70.2

		2855		68.43

		2854		66.63

		2853		64.87

		2852		63.26

		2851		61.88

		2850		60.82

		2849		60.16

		2848		59.96

		2847		60.22

		2846		60.92

		2845		62.03

		2844		63.48

		2843		65.17

		2842		67.02

		2841		68.95

		2840		70.88

		2839		72.72

		2838		74.43

		2837		75.98

		2836		77.35

		2835		78.54

		2834		79.56

		2833		80.44

		2832		81.2

		2831		81.85

		2830		82.42

		2829		82.92

		2828		83.36

		2827		83.75

		2826		84.1

		2825		84.42

		2824		84.71

		2823		84.97

		2822		85.21

		2821		85.43

		2820		85.64

		2819		85.83

		2818		86

		2817		86.17

		2816		86.32

		2815		86.46

		2814		86.59

		2813		86.72

		2812		86.84

		2811		86.95

		2810		87.06

		2809		87.16

		2808		87.26

		2807		87.35

		2806		87.45

		2805		87.54

		2804		87.62

		2803		87.71

		2802		87.79

		2801		87.87

		2800		87.94

		2799		88.02

		2798		88.09

		2797		88.16

		2796		88.22

		2795		88.28

		2794		88.34

		2793		88.39

		2792		88.45

		2791		88.49

		2790		88.54

		2789		88.58

		2788		88.63

		2787		88.66

		2786		88.7

		2785		88.74

		2784		88.77

		2783		88.8

		2782		88.83

		2781		88.86

		2780		88.89

		2779		88.91

		2778		88.94

		2777		88.96

		2776		88.99

		2775		89.01

		2774		89.03

		2773		89.05

		2772		89.07

		2771		89.1

		2770		89.12

		2769		89.14

		2768		89.16

		2767		89.18

		2766		89.2

		2765		89.23

		2764		89.25

		2763		89.27

		2762		89.3

		2761		89.32

		2760		89.34

		2759		89.37

		2758		89.39

		2757		89.41

		2756		89.44

		2755		89.46

		2754		89.48

		2753		89.5

		2752		89.53

		2751		89.55

		2750		89.57

		2749		89.6

		2748		89.62

		2747		89.65

		2746		89.67

		2745		89.7

		2744		89.73

		2743		89.75

		2742		89.77

		2741		89.79

		2740		89.81

		2739		89.83

		2738		89.85

		2737		89.87

		2736		89.88

		2735		89.89

		2734		89.91

		2733		89.92

		2732		89.93

		2731		89.94

		2730		89.95

		2729		89.97

		2728		89.98

		2727		89.99

		2726		90

		2725		90.01

		2724		90.02

		2723		90.03

		2722		90.03

		2721		90.03

		2720		90.02

		2719		90.02

		2718		90

		2717		89.98

		2716		89.96

		2715		89.93

		2714		89.9

		2713		89.87

		2712		89.84

		2711		89.8

		2710		89.77

		2709		89.74

		2708		89.7

		2707		89.67

		2706		89.65

		2705		89.62

		2704		89.59

		2703		89.57

		2702		89.55

		2701		89.53

		2700		89.51

		2699		89.49

		2698		89.47

		2697		89.45

		2696		89.43

		2695		89.4

		2694		89.38

		2693		89.35

		2692		89.33

		2691		89.3

		2690		89.28

		2689		89.25

		2688		89.22

		2687		89.2

		2686		89.18

		2685		89.16

		2684		89.14

		2683		89.12

		2682		89.11

		2681		89.1

		2680		89.09

		2679		89.09

		2678		89.08

		2677		89.08

		2676		89.08

		2675		89.08

		2674		89.08

		2673		89.08

		2672		89.08

		2671		89.09

		2670		89.09

		2669		89.09

		2668		89.09

		2667		89.1

		2666		89.1

		2665		89.1

		2664		89.1

		2663		89.1

		2662		89.1

		2661		89.09

		2660		89.09

		2659		89.09

		2658		89.08

		2657		89.08

		2656		89.08

		2655		89.07

		2654		89.07

		2653		89.07

		2652		89.07

		2651		89.08

		2650		89.08

		2649		89.09

		2648		89.1

		2647		89.11

		2646		89.12

		2645		89.14

		2644		89.15

		2643		89.16

		2642		89.18

		2641		89.19

		2640		89.2

		2639		89.21

		2638		89.22

		2637		89.22

		2636		89.23

		2635		89.23

		2634		89.24

		2633		89.24

		2632		89.25

		2631		89.26

		2630		89.27

		2629		89.29

		2628		89.3

		2627		89.32

		2626		89.35

		2625		89.38

		2624		89.41

		2623		89.44

		2622		89.47

		2621		89.5

		2620		89.53

		2619		89.56

		2618		89.58

		2617		89.61

		2616		89.63

		2615		89.64

		2614		89.66

		2613		89.67

		2612		89.69

		2611		89.7

		2610		89.71

		2609		89.73

		2608		89.74

		2607		89.76

		2606		89.78

		2605		89.8

		2604		89.82

		2603		89.85

		2602		89.87

		2601		89.9

		2600		89.93

		2599		89.97

		2598		90

		2597		90.03

		2596		90.06

		2595		90.1

		2594		90.13

		2593		90.16

		2592		90.19

		2591		90.21

		2590		90.24

		2589		90.26

		2588		90.28

		2587		90.3

		2586		90.32

		2585		90.33

		2584		90.35

		2583		90.36

		2582		90.38

		2581		90.39

		2580		90.4

		2579		90.41

		2578		90.42

		2577		90.43

		2576		90.44

		2575		90.45

		2574		90.46

		2573		90.47

		2572		90.48

		2571		90.48

		2570		90.49

		2569		90.49

		2568		90.49

		2567		90.49

		2566		90.49

		2565		90.49

		2564		90.49

		2563		90.49

		2562		90.5

		2561		90.5

		2560		90.51

		2559		90.52

		2558		90.53

		2557		90.55

		2556		90.57

		2555		90.6

		2554		90.63

		2553		90.66

		2552		90.7

		2551		90.74

		2550		90.78

		2549		90.82

		2548		90.86

		2547		90.9

		2546		90.94

		2545		90.98

		2544		91.02

		2543		91.05

		2542		91.07

		2541		91.09

		2540		91.11

		2539		91.13

		2538		91.14

		2537		91.15

		2536		91.16

		2535		91.17

		2534		91.19

		2533		91.2

		2532		91.23

		2531		91.26

		2530		91.3

		2529		91.34

		2528		91.39

		2527		91.44

		2526		91.5

		2525		91.56

		2524		91.62

		2523		91.68

		2522		91.74

		2521		91.79

		2520		91.84

		2519		91.89

		2518		91.93

		2517		91.97

		2516		92.01

		2515		92.04

		2514		92.07

		2513		92.1

		2512		92.13

		2511		92.17

		2510		92.2

		2509		92.24

		2508		92.28

		2507		92.32

		2506		92.37

		2505		92.41

		2504		92.45

		2503		92.5

		2502		92.54

		2501		92.58

		2500		92.62

		2499		92.65

		2498		92.69

		2497		92.71

		2496		92.74

		2495		92.76

		2494		92.78

		2493		92.79

		2492		92.81

		2491		92.83

		2490		92.84

		2489		92.86

		2488		92.88

		2487		92.91

		2486		92.94

		2485		92.97

		2484		93.01

		2483		93.04

		2482		93.08

		2481		93.12

		2480		93.16

		2479		93.2

		2478		93.23

		2477		93.26

		2476		93.29

		2475		93.32

		2474		93.34

		2473		93.36

		2472		93.38

		2471		93.4

		2470		93.41

		2469		93.43

		2468		93.44

		2467		93.45

		2466		93.47

		2465		93.48

		2464		93.5

		2463		93.52

		2462		93.54

		2461		93.56

		2460		93.58

		2459		93.61

		2458		93.63

		2457		93.66

		2456		93.68

		2455		93.71

		2454		93.73

		2453		93.75

		2452		93.77

		2451		93.79

		2450		93.81

		2449		93.82

		2448		93.83

		2447		93.85

		2446		93.86

		2445		93.87

		2444		93.89

		2443		93.9

		2442		93.92

		2441		93.94

		2440		93.96

		2439		93.98

		2438		94

		2437		94.02

		2436		94.05

		2435		94.07

		2434		94.1

		2433		94.12

		2432		94.14

		2431		94.17

		2430		94.19

		2429		94.21

		2428		94.22

		2427		94.24

		2426		94.25

		2425		94.27

		2424		94.28

		2423		94.29

		2422		94.3

		2421		94.31

		2420		94.32

		2419		94.33

		2418		94.34

		2417		94.36

		2416		94.37

		2415		94.39

		2414		94.41

		2413		94.42

		2412		94.44

		2411		94.46

		2410		94.47

		2409		94.49

		2408		94.5

		2407		94.52

		2406		94.53

		2405		94.54

		2404		94.55

		2403		94.56

		2402		94.58

		2401		94.59

		2400		94.6

		2399		94.61

		2398		94.62

		2397		94.63

		2396		94.64

		2395		94.65

		2394		94.66

		2393		94.67

		2392		94.69

		2391		94.7

		2390		94.72

		2389		94.73

		2388		94.75

		2387		94.77

		2386		94.79

		2385		94.81

		2384		94.82

		2383		94.84

		2382		94.85

		2381		94.87

		2380		94.88

		2379		94.89

		2378		94.89

		2377		94.9

		2376		94.9

		2375		94.91

		2374		94.91

		2373		94.92

		2372		94.93

		2371		94.93

		2370		94.94

		2369		94.94

		2368		94.94

		2367		94.95

		2366		94.95

		2365		94.95

		2364		94.95

		2363		94.95

		2362		94.95

		2361		94.95

		2360		94.96

		2359		94.96

		2358		94.97

		2357		94.97

		2356		94.98

		2355		94.98

		2354		94.98

		2353		94.99

		2352		94.99

		2351		94.99

		2350		94.98

		2349		94.98

		2348		94.97

		2347		94.97

		2346		94.97

		2345		94.97

		2344		94.97

		2343		94.97

		2342		94.98

		2341		94.98

		2340		94.99

		2339		95

		2338		95

		2337		95.01

		2336		95.02

		2335		95.02

		2334		95.02

		2333		95.02

		2332		95.02

		2331		95.01

		2330		95.01

		2329		95

		2328		94.99

		2327		94.98

		2326		94.97

		2325		94.97

		2324		94.97

		2323		94.97

		2322		94.98

		2321		94.99

		2320		95

		2319		95.02

		2318		95.04

		2317		95.06

		2316		95.08

		2315		95.1

		2314		95.12

		2313		95.14

		2312		95.16

		2311		95.18

		2310		95.2

		2309		95.22

		2308		95.23

		2307		95.24

		2306		95.25

		2305		95.26

		2304		95.26

		2303		95.26

		2302		95.26

		2301		95.26

		2300		95.26

		2299		95.25

		2298		95.25

		2297		95.24

		2296		95.23

		2295		95.22

		2294		95.21

		2293		95.2

		2292		95.19

		2291		95.18

		2290		95.17

		2289		95.17

		2288		95.16

		2287		95.16

		2286		95.16

		2285		95.16

		2284		95.17

		2283		95.18

		2282		95.19

		2281		95.2

		2280		95.21

		2279		95.23

		2278		95.24

		2277		95.26

		2276		95.27

		2275		95.29

		2274		95.3

		2273		95.31

		2272		95.33

		2271		95.34

		2270		95.35

		2269		95.36

		2268		95.37

		2267		95.38

		2266		95.39

		2265		95.4

		2264		95.41

		2263		95.42

		2262		95.43

		2261		95.44

		2260		95.45

		2259		95.47

		2258		95.48

		2257		95.5

		2256		95.52

		2255		95.54

		2254		95.56

		2253		95.57

		2252		95.59

		2251		95.61

		2250		95.63

		2249		95.64

		2248		95.65

		2247		95.66

		2246		95.67

		2245		95.68

		2244		95.69

		2243		95.7

		2242		95.71

		2241		95.72

		2240		95.73

		2239		95.74

		2238		95.75

		2237		95.77

		2236		95.78

		2235		95.79

		2234		95.8

		2233		95.81

		2232		95.82

		2231		95.84

		2230		95.85

		2229		95.86

		2228		95.86

		2227		95.87

		2226		95.89

		2225		95.9

		2224		95.91

		2223		95.92

		2222		95.93

		2221		95.93

		2220		95.94

		2219		95.94

		2218		95.95

		2217		95.95

		2216		95.94

		2215		95.94

		2214		95.94

		2213		95.94

		2212		95.93

		2211		95.93

		2210		95.93

		2209		95.93

		2208		95.93

		2207		95.93

		2206		95.94

		2205		95.94

		2204		95.94

		2203		95.94

		2202		95.94

		2201		95.94

		2200		95.94

		2199		95.94

		2198		95.93

		2197		95.93

		2196		95.93

		2195		95.92

		2194		95.92

		2193		95.92

		2192		95.92

		2191		95.92

		2190		95.93

		2189		95.93

		2188		95.94

		2187		95.95

		2186		95.96

		2185		95.97

		2184		95.99

		2183		96

		2182		96.01

		2181		96.03

		2180		96.04

		2179		96.05

		2178		96.05

		2177		96.06

		2176		96.06

		2175		96.06

		2174		96.06

		2173		96.05

		2172		96.03

		2171		96.02

		2170		96

		2169		95.99

		2168		95.99

		2167		96

		2166		96.01

		2165		96.04

		2164		96.07

		2163		96.12

		2162		96.17

		2161		96.23

		2160		96.3

		2159		96.36

		2158		96.41

		2157		96.46

		2156		96.49

		2155		96.51

		2154		96.52

		2153		96.53

		2152		96.52

		2151		96.51

		2150		96.5

		2149		96.48

		2148		96.47

		2147		96.45

		2146		96.45

		2145		96.44

		2144		96.44

		2143		96.44

		2142		96.44

		2141		96.44

		2140		96.44

		2139		96.45

		2138		96.45

		2137		96.45

		2136		96.46

		2135		96.46

		2134		96.45

		2133		96.45

		2132		96.44

		2131		96.43

		2130		96.42

		2129		96.4

		2128		96.39

		2127		96.37

		2126		96.35

		2125		96.34

		2124		96.32

		2123		96.3

		2122		96.28

		2121		96.27

		2120		96.25

		2119		96.23

		2118		96.22

		2117		96.21

		2116		96.19

		2115		96.19

		2114		96.18

		2113		96.18

		2112		96.17

		2111		96.17

		2110		96.17

		2109		96.18

		2108		96.18

		2107		96.18

		2106		96.18

		2105		96.18

		2104		96.18

		2103		96.19

		2102		96.19

		2101		96.19

		2100		96.2

		2099		96.2

		2098		96.21

		2097		96.22

		2096		96.22

		2095		96.23

		2094		96.23

		2093		96.23

		2092		96.23

		2091		96.23

		2090		96.23

		2089		96.23

		2088		96.22

		2087		96.21

		2086		96.2

		2085		96.19

		2084		96.18

		2083		96.18

		2082		96.17

		2081		96.17

		2080		96.17

		2079		96.18

		2078		96.18

		2077		96.19

		2076		96.2

		2075		96.21

		2074		96.22

		2073		96.23

		2072		96.25

		2071		96.26

		2070		96.27

		2069		96.28

		2068		96.28

		2067		96.29

		2066		96.3

		2065		96.3

		2064		96.31

		2063		96.31

		2062		96.32

		2061		96.32

		2060		96.32

		2059		96.32

		2058		96.31

		2057		96.31

		2056		96.3

		2055		96.3

		2054		96.29

		2053		96.28

		2052		96.28

		2051		96.28

		2050		96.28

		2049		96.29

		2048		96.3

		2047		96.31

		2046		96.31

		2045		96.32

		2044		96.33

		2043		96.34

		2042		96.35

		2041		96.36

		2040		96.37

		2039		96.38

		2038		96.39

		2037		96.4

		2036		96.4

		2035		96.42

		2034		96.43

		2033		96.44

		2032		96.45

		2031		96.46

		2030		96.47

		2029		96.47

		2028		96.48

		2027		96.48

		2026		96.48

		2025		96.48

		2024		96.47

		2023		96.47

		2022		96.46

		2021		96.46

		2020		96.46

		2019		96.46

		2018		96.46

		2017		96.46

		2016		96.47

		2015		96.48

		2014		96.49

		2013		96.51

		2012		96.52

		2011		96.54

		2010		96.56

		2009		96.58

		2008		96.6

		2007		96.61

		2006		96.62

		2005		96.62

		2004		96.62

		2003		96.61

		2002		96.6

		2001		96.58

		2000		96.56

		1999		96.54

		1998		96.52

		1997		96.49

		1996		96.47

		1995		96.45

		1994		96.43

		1993		96.41

		1992		96.39

		1991		96.38

		1990		96.36

		1989		96.34

		1988		96.33

		1987		96.32

		1986		96.31

		1985		96.3

		1984		96.3

		1983		96.31

		1982		96.32

		1981		96.34

		1980		96.36

		1979		96.39

		1978		96.43

		1977		96.46

		1976		96.49

		1975		96.52

		1974		96.55

		1973		96.57

		1972		96.58

		1971		96.6

		1970		96.6

		1969		96.61

		1968		96.61

		1967		96.61

		1966		96.61

		1965		96.6

		1964		96.6

		1963		96.6

		1962		96.6

		1961		96.59

		1960		96.58

		1959		96.58

		1958		96.57

		1957		96.55

		1956		96.54

		1955		96.53

		1954		96.51

		1953		96.5

		1952		96.49

		1951		96.48

		1950		96.47

		1949		96.46

		1948		96.46

		1947		96.46

		1946		96.46

		1945		96.46

		1944		96.45

		1943		96.45

		1942		96.45

		1941		96.45

		1940		96.45

		1939		96.44

		1938		96.44

		1937		96.44

		1936		96.43

		1935		96.42

		1934		96.42

		1933		96.41

		1932		96.41

		1931		96.4

		1930		96.4

		1929		96.39

		1928		96.38

		1927		96.37

		1926		96.36

		1925		96.35

		1924		96.34

		1923		96.32

		1922		96.31

		1921		96.3

		1920		96.29

		1919		96.28

		1918		96.27

		1917		96.26

		1916		96.25

		1915		96.25

		1914		96.24

		1913		96.24

		1912		96.24

		1911		96.24

		1910		96.24

		1909		96.24

		1908		96.23

		1907		96.22

		1906		96.22

		1905		96.2

		1904		96.19

		1903		96.17

		1902		96.16

		1901		96.14

		1900		96.13

		1899		96.11

		1898		96.1

		1897		96.1

		1896		96.09

		1895		96.09

		1894		96.09

		1893		96.09

		1892		96.09

		1891		96.09

		1890		96.09

		1889		96.09

		1888		96.09

		1887		96.08

		1886		96.07

		1885		96.07

		1884		96.06

		1883		96.05

		1882		96.04

		1881		96.02

		1880		96.01

		1879		96

		1878		95.99

		1877		95.98

		1876		95.97

		1875		95.96

		1874		95.95

		1873		95.94

		1872		95.93

		1871		95.92

		1870		95.91

		1869		95.9

		1868		95.89

		1867		95.88

		1866		95.87

		1865		95.86

		1864		95.85

		1863		95.83

		1862		95.82

		1861		95.81

		1860		95.79

		1859		95.78

		1858		95.76

		1857		95.75

		1856		95.73

		1855		95.72

		1854		95.7

		1853		95.69

		1852		95.67

		1851		95.65

		1850		95.64

		1849		95.63

		1848		95.61

		1847		95.6

		1846		95.59

		1845		95.58

		1844		95.56

		1843		95.55

		1842		95.54

		1841		95.53

		1840		95.52

		1839		95.51

		1838		95.51

		1837		95.5

		1836		95.49

		1835		95.48

		1834		95.47

		1833		95.46

		1832		95.45

		1831		95.44

		1830		95.42

		1829		95.4

		1828		95.38

		1827		95.36

		1826		95.33

		1825		95.31

		1824		95.28

		1823		95.26

		1822		95.23

		1821		95.21

		1820		95.18

		1819		95.16

		1818		95.14

		1817		95.13

		1816		95.11

		1815		95.1

		1814		95.08

		1813		95.07

		1812		95.06

		1811		95.05

		1810		95.04

		1809		95.03

		1808		95.02

		1807		95.01

		1806		95

		1805		94.98

		1804		94.97

		1803		94.95

		1802		94.93

		1801		94.91

		1800		94.88

		1799		94.85

		1798		94.81

		1797		94.77

		1796		94.73

		1795		94.68

		1794		94.63

		1793		94.58

		1792		94.53

		1791		94.48

		1790		94.44

		1789		94.4

		1788		94.36

		1787		94.34

		1786		94.32

		1785		94.31

		1784		94.32

		1783		94.33

		1782		94.35

		1781		94.39

		1780		94.42

		1779		94.47

		1778		94.51

		1777		94.56

		1776		94.6

		1775		94.65

		1774		94.69

		1773		94.74

		1772		94.77

		1771		94.81

		1770		94.84

		1769		94.87

		1768		94.9

		1767		94.93

		1766		94.95

		1765		94.98

		1764		95

		1763		95.02

		1762		95.04

		1761		95.06

		1760		95.07

		1759		95.09

		1758		95.1

		1757		95.11

		1756		95.11

		1755		95.11

		1754		95.11

		1753		95.1

		1752		95.09

		1751		95.08

		1750		95.06

		1749		95.03

		1748		95

		1747		94.95

		1746		94.91

		1745		94.85

		1744		94.79

		1743		94.71

		1742		94.63

		1741		94.53

		1740		94.42

		1739		94.29

		1738		94.16

		1737		94.01

		1736		93.83

		1735		93.64

		1734		93.43

		1733		93.19

		1732		92.92

		1731		92.62

		1730		92.28

		1729		91.89

		1728		91.45

		1727		90.95

		1726		90.36

		1725		89.69

		1724		88.91

		1723		88.04

		1722		87.06

		1721		85.96

		1720		84.76

		1719		83.44

		1718		82.02

		1717		80.5

		1716		78.91

		1715		77.24

		1714		75.5

		1713		73.69

		1712		71.84

		1711		69.94

		1710		68

		1709		66.03

		1708		64.06

		1707		62.09

		1706		60.16

		1705		58.3

		1704		56.55

		1703		54.94

		1702		53.49

		1701		52.22

		1700		51.15

		1699		50.29

		1698		49.67

		1697		49.26

		1696		49.04

		1695		49

		1694		49.1

		1693		49.33

		1692		49.7

		1691		50.18

		1690		50.78

		1689		51.49

		1688		52.32

		1687		53.26

		1686		54.35

		1685		55.58

		1684		56.98

		1683		58.52

		1682		60.2

		1681		61.99

		1680		63.88

		1679		65.84

		1678		67.83

		1677		69.82

		1676		71.78

		1675		73.68

		1674		75.48

		1673		77.17

		1672		78.73

		1671		80.16

		1670		81.47

		1669		82.64

		1668		83.7

		1667		84.63

		1666		85.45

		1665		86.18

		1664		86.83

		1663		87.42

		1662		87.94

		1661		88.4

		1660		88.82

		1659		89.19

		1658		89.53

		1657		89.84

		1656		90.12

		1655		90.38

		1654		90.61

		1653		90.83

		1652		91.03

		1651		91.22

		1650		91.39

		1649		91.56

		1648		91.71

		1647		91.86

		1646		92.01

		1645		92.14

		1644		92.27

		1643		92.4

		1642		92.52

		1641		92.64

		1640		92.76

		1639		92.87

		1638		92.98

		1637		93.08

		1636		93.18

		1635		93.28

		1634		93.38

		1633		93.47

		1632		93.56

		1631		93.65

		1630		93.73

		1629		93.81

		1628		93.89

		1627		93.97

		1626		94.04

		1625		94.12

		1624		94.19

		1623		94.26

		1622		94.33

		1621		94.4

		1620		94.46

		1619		94.53

		1618		94.6

		1617		94.66

		1616		94.72

		1615		94.78

		1614		94.84

		1613		94.9

		1612		94.95

		1611		95

		1610		95.05

		1609		95.1

		1608		95.14

		1607		95.18

		1606		95.22

		1605		95.25

		1604		95.28

		1603		95.31

		1602		95.33

		1601		95.36

		1600		95.38

		1599		95.4

		1598		95.42

		1597		95.44

		1596		95.46

		1595		95.48

		1594		95.5

		1593		95.52

		1592		95.54

		1591		95.56

		1590		95.58

		1589		95.6

		1588		95.62

		1587		95.63

		1586		95.65

		1585		95.67

		1584		95.68

		1583		95.69

		1582		95.7

		1581		95.71

		1580		95.72

		1579		95.72

		1578		95.73

		1577		95.73

		1576		95.73

		1575		95.73

		1574		95.73

		1573		95.73

		1572		95.72

		1571		95.72

		1570		95.72

		1569		95.72

		1568		95.72

		1567		95.72

		1566		95.72

		1565		95.72

		1564		95.73

		1563		95.73

		1562		95.74

		1561		95.74

		1560		95.75

		1559		95.76

		1558		95.76

		1557		95.77

		1556		95.77

		1555		95.78

		1554		95.78

		1553		95.79

		1552		95.79

		1551		95.8

		1550		95.8

		1549		95.81

		1548		95.81

		1547		95.81

		1546		95.81

		1545		95.82

		1544		95.82

		1543		95.82

		1542		95.83

		1541		95.83

		1540		95.84

		1539		95.84

		1538		95.85

		1537		95.86

		1536		95.86

		1535		95.86

		1534		95.86

		1533		95.86

		1532		95.86

		1531		95.86

		1530		95.86

		1529		95.85

		1528		95.84

		1527		95.83

		1526		95.82

		1525		95.81

		1524		95.8

		1523		95.78

		1522		95.77

		1521		95.76

		1520		95.75

		1519		95.73

		1518		95.72

		1517		95.71

		1516		95.7

		1515		95.68

		1514		95.67

		1513		95.66

		1512		95.65

		1511		95.64

		1510		95.64

		1509		95.63

		1508		95.62

		1507		95.61

		1506		95.61

		1505		95.6

		1504		95.59

		1503		95.58

		1502		95.57

		1501		95.56

		1500		95.54

		1499		95.53

		1498		95.51

		1497		95.49

		1496		95.46

		1495		95.44

		1494		95.41

		1493		95.38

		1492		95.35

		1491		95.31

		1490		95.26

		1489		95.2

		1488		95.13

		1487		95.04

		1486		94.92

		1485		94.75

		1484		94.51

		1483		94.17

		1482		93.67

		1481		93

		1480		92.16

		1479		91.17

		1478		90.06

		1477		88.85

		1476		87.59

		1475		86.29

		1474		85

		1473		83.8

		1472		82.78

		1471		81.99

		1470		81.46

		1469		81.16

		1468		81.03

		1467		81.05

		1466		81.19

		1465		81.44

		1464		81.81

		1463		82.26

		1462		82.75

		1461		83.23

		1460		83.69

		1459		84.13

		1458		84.57

		1457		85.01

		1456		85.44

		1455		85.86

		1454		86.23

		1453		86.55

		1452		86.79

		1451		86.97

		1450		87.08

		1449		87.12

		1448		87.1

		1447		87.01

		1446		86.86

		1445		86.65

		1444		86.38

		1443		86.06

		1442		85.69

		1441		85.26

		1440		84.78

		1439		84.26

		1438		83.7

		1437		83.11

		1436		82.52

		1435		81.94

		1434		81.41

		1433		80.94

		1432		80.57

		1431		80.3

		1430		80.16

		1429		80.16

		1428		80.3

		1427		80.57

		1426		80.94

		1425		81.38

		1424		81.86

		1423		82.34

		1422		82.77

		1421		83.12

		1420		83.36

		1419		83.49

		1418		83.48

		1417		83.36

		1416		83.14

		1415		82.85

		1414		82.54

		1413		82.25

		1412		82.04

		1411		81.94

		1410		81.98

		1409		82.18

		1408		82.55

		1407		83.06

		1406		83.71

		1405		84.47

		1404		85.3

		1403		86.17

		1402		87.03

		1401		87.87

		1400		88.65

		1399		89.36

		1398		89.98

		1397		90.53

		1396		91

		1395		91.39

		1394		91.72

		1393		91.99

		1392		92.21

		1391		92.4

		1390		92.54

		1389		92.65

		1388		92.72

		1387		92.77

		1386		92.79

		1385		92.78

		1384		92.75

		1383		92.69

		1382		92.61

		1381		92.51

		1380		92.4

		1379		92.28

		1378		92.16

		1377		92.04

		1376		91.93

		1375		91.83

		1374		91.74

		1373		91.66

		1372		91.6

		1371		91.54

		1370		91.49

		1369		91.42

		1368		91.34

		1367		91.23

		1366		91.1

		1365		90.94

		1364		90.75

		1363		90.54

		1362		90.31

		1361		90.06

		1360		89.81

		1359		89.56

		1358		89.31

		1357		89.09

		1356		88.89

		1355		88.73

		1354		88.6

		1353		88.51

		1352		88.46

		1351		88.47

		1350		88.53

		1349		88.65

		1348		88.82

		1347		89.04

		1346		89.29

		1345		89.57

		1344		89.85

		1343		90.12

		1342		90.35

		1341		90.52

		1340		90.61

		1339		90.61

		1338		90.52

		1337		90.34

		1336		90.08

		1335		89.76

		1334		89.4

		1333		89.02

		1332		88.66

		1331		88.35

		1330		88.11

		1329		87.96

		1328		87.89

		1327		87.9

		1326		87.98

		1325		88.08

		1324		88.2

		1323		88.27

		1322		88.28

		1321		88.17

		1320		87.91

		1319		87.49

		1318		86.9

		1317		86.14

		1316		85.23

		1315		84.19

		1314		83.07

		1313		81.9

		1312		80.75

		1311		79.64

		1310		78.64

		1309		77.77

		1308		77.07

		1307		76.55

		1306		76.19

		1305		75.99

		1304		75.92

		1303		75.94

		1302		76.02

		1301		76.12

		1300		76.22

		1299		76.28

		1298		76.25

		1297		76.12

		1296		75.88

		1295		75.54

		1294		75.14

		1293		74.69

		1292		74.24

		1291		73.81

		1290		73.45

		1289		73.2

		1288		73.09

		1287		73.17

		1286		73.47

		1285		74

		1284		74.74

		1283		75.67

		1282		76.75

		1281		77.93

		1280		79.17

		1279		80.42

		1278		81.63

		1277		82.76

		1276		83.77

		1275		84.61

		1274		85.26

		1273		85.7

		1272		85.92

		1271		85.94

		1270		85.78

		1269		85.46

		1268		85.01

		1267		84.49

		1266		83.93

		1265		83.39

		1264		82.93

		1263		82.6

		1262		82.46

		1261		82.52

		1260		82.79

		1259		83.25

		1258		83.88

		1257		84.62

		1256		85.45

		1255		86.31

		1254		87.16

		1253		87.94

		1252		88.62

		1251		89.17

		1250		89.54

		1249		89.73

		1248		89.71

		1247		89.49

		1246		89.05

		1245		88.44

		1244		87.68

		1243		86.8

		1242		85.85

		1241		84.88

		1240		83.96

		1239		83.17

		1238		82.57

		1237		82.22

		1236		82.15

		1235		82.34

		1234		82.77

		1233		83.4

		1232		84.17

		1231		85.05

		1230		85.96

		1229		86.85

		1228		87.66

		1227		88.33

		1226		88.83

		1225		89.14

		1224		89.24

		1223		89.16

		1222		88.9

		1221		88.48

		1220		87.93

		1219		87.29

		1218		86.58

		1217		85.86

		1216		85.17

		1215		84.57

		1214		84.11

		1213		83.84

		1212		83.77

		1211		83.9

		1210		84.22

		1209		84.71

		1208		85.35

		1207		86.09

		1206		86.89

		1205		87.7

		1204		88.45

		1203		89.09

		1202		89.57

		1201		89.86

		1200		89.94

		1199		89.81

		1198		89.5

		1197		89.03

		1196		88.45

		1195		87.8

		1194		87.14

		1193		86.52

		1192		86.02

		1191		85.69

		1190		85.59

		1189		85.72

		1188		86.06

		1187		86.59

		1186		87.25

		1185		88

		1184		88.81

		1183		89.62

		1182		90.41

		1181		91.13

		1180		91.76

		1179		92.29

		1178		92.71

		1177		93.05

		1176		93.33

		1175		93.56

		1174		93.74

		1173		93.9

		1172		94.04

		1171		94.16

		1170		94.26

		1169		94.36

		1168		94.44

		1167		94.51

		1166		94.58

		1165		94.64

		1164		94.7

		1163		94.75

		1162		94.79

		1161		94.84

		1160		94.88

		1159		94.91

		1158		94.95

		1157		94.98

		1156		95.01

		1155		95.04

		1154		95.06

		1153		95.08

		1152		95.11

		1151		95.13

		1150		95.14

		1149		95.16

		1148		95.18

		1147		95.19

		1146		95.2

		1145		95.22

		1144		95.22

		1143		95.23

		1142		95.24

		1141		95.24

		1140		95.23

		1139		95.22

		1138		95.2

		1137		95.17

		1136		95.12

		1135		95.06

		1134		94.98

		1133		94.88

		1132		94.76

		1131		94.63

		1130		94.49

		1129		94.34

		1128		94.2

		1127		94.07

		1126		93.95

		1125		93.87

		1124		93.81

		1123		93.79

		1122		93.81

		1121		93.85

		1120		93.92

		1119		94

		1118		94.09

		1117		94.18

		1116		94.27

		1115		94.35

		1114		94.41

		1113		94.46

		1112		94.49

		1111		94.51

		1110		94.52

		1109		94.53

		1108		94.52

		1107		94.5

		1106		94.47

		1105		94.41

		1104		94.31

		1103		94.16

		1102		93.94

		1101		93.67

		1100		93.33

		1099		92.95

		1098		92.55

		1097		92.13

		1096		91.71

		1095		91.33

		1094		91.02

		1093		90.79

		1092		90.68

		1091		90.68

		1090		90.78

		1089		90.97

		1088		91.21

		1087		91.5

		1086		91.8

		1085		92.1

		1084		92.38

		1083		92.63

		1082		92.82

		1081		92.97

		1080		93.07

		1079		93.13

		1078		93.17

		1077		93.18

		1076		93.18

		1075		93.17

		1074		93.15

		1073		93.12

		1072		93.08

		1071		93.05

		1070		93

		1069		92.95

		1068		92.9

		1067		92.85

		1066		92.8

		1065		92.76

		1064		92.72

		1063		92.68

		1062		92.64

		1061		92.6

		1060		92.56

		1059		92.53

		1058		92.5

		1057		92.47

		1056		92.45

		1055		92.43

		1054		92.42

		1053		92.42

		1052		92.42

		1051		92.43

		1050		92.45

		1049		92.47

		1048		92.48

		1047		92.5

		1046		92.5

		1045		92.5

		1044		92.49

		1043		92.47

		1042		92.45

		1041		92.42

		1040		92.4

		1039		92.39

		1038		92.39

		1037		92.4

		1036		92.43

		1035		92.47

		1034		92.52

		1033		92.58

		1032		92.66

		1031		92.74

		1030		92.81

		1029		92.88

		1028		92.93

		1027		92.97

		1026		93

		1025		93.02

		1024		93.03

		1023		93.03

		1022		93.02

		1021		93

		1020		92.98

		1019		92.96

		1018		92.94

		1017		92.92

		1016		92.89

		1015		92.86

		1014		92.84

		1013		92.8

		1012		92.77

		1011		92.73

		1010		92.68

		1009		92.63

		1008		92.57

		1007		92.51

		1006		92.45

		1005		92.38

		1004		92.32

		1003		92.27

		1002		92.22

		1001		92.19

		1000		92.17

		999		92.16

		998		92.16

		997		92.18

		996		92.19

		995		92.21

		994		92.21

		993		92.21

		992		92.19

		991		92.16

		990		92.12

		989		92.06

		988		91.99

		987		91.91

		986		91.83

		985		91.75

		984		91.67

		983		91.58

		982		91.49

		981		91.38

		980		91.25

		979		91.11

		978		90.93

		977		90.73

		976		90.48

		975		90.21

		974		89.89

		973		89.54

		972		89.16

		971		88.75

		970		88.31

		969		87.86

		968		87.4

		967		86.93

		966		86.45

		965		85.97

		964		85.48

		963		84.99

		962		84.5

		961		84.02

		960		83.53

		959		83.05

		958		82.56

		957		82.06

		956		81.56

		955		81.06

		954		80.54

		953		80

		952		79.45

		951		78.88

		950		78.3

		949		77.69

		948		77.08

		947		76.46

		946		75.85

		945		75.27

		944		74.71

		943		74.21

		942		73.78

		941		73.43

		940		73.18

		939		73.03

		938		72.99

		937		73.07

		936		73.27

		935		73.57

		934		73.98

		933		74.48

		932		75.06

		931		75.71

		930		76.41

		929		77.14

		928		77.9

		927		78.67

		926		79.43

		925		80.17

		924		80.88

		923		81.55

		922		82.17

		921		82.72

		920		83.2

		919		83.62

		918		83.96

		917		84.22

		916		84.42

		915		84.55

		914		84.64

		913		84.7

		912		84.74

		911		84.78

		910		84.84

		909		84.93

		908		85.05

		907		85.21

		906		85.41

		905		85.63

		904		85.88

		903		86.12

		902		86.35

		901		86.55

		900		86.71

		899		86.81

		898		86.87

		897		86.87

		896		86.83

		895		86.76

		894		86.66

		893		86.57

		892		86.5

		891		86.46

		890		86.45

		889		86.49

		888		86.59

		887		86.74

		886		86.94

		885		87.19

		884		87.47

		883		87.77

		882		88.08

		881		88.39

		880		88.69

		879		88.98

		878		89.26

		877		89.52

		876		89.76

		875		89.98

		874		90.18

		873		90.37

		872		90.55

		871		90.72

		870		90.88

		869		91.03

		868		91.18

		867		91.32

		866		91.46

		865		91.59

		864		91.72

		863		91.85

		862		91.97

		861		92.1

		860		92.24

		859		92.37

		858		92.52

		857		92.66

		856		92.8

		855		92.95

		854		93.09

		853		93.23

		852		93.36

		851		93.48

		850		93.6

		849		93.71

		848		93.81

		847		93.91

		846		93.99

		845		94.07

		844		94.15

		843		94.22

		842		94.29

		841		94.35

		840		94.41

		839		94.47

		838		94.52

		837		94.57

		836		94.62

		835		94.66

		834		94.71

		833		94.74

		832		94.77

		831		94.8

		830		94.82

		829		94.83

		828		94.83

		827		94.8

		826		94.75

		825		94.66

		824		94.53

		823		94.36

		822		94.17

		821		93.96

		820		93.74

		819		93.53

		818		93.34

		817		93.18

		816		93.09

		815		93.06

		814		93.12

		813		93.26

		812		93.46

		811		93.72

		810		94

		809		94.3

		808		94.59

		807		94.87

		806		95.13

		805		95.35

		804		95.53

		803		95.67

		802		95.77

		801		95.84

		800		95.9

		799		95.94

		798		95.97

		797		96

		796		96.02

		795		96.03

		794		96.03

		793		96.02

		792		95.99

		791		95.94

		790		95.87

		789		95.79

		788		95.69

		787		95.59

		786		95.49

		785		95.39

		784		95.31

		783		95.24

		782		95.21

		781		95.2

		780		95.24

		779		95.3

		778		95.39

		777		95.5

		776		95.61

		775		95.73

		774		95.84

		773		95.94

		772		96.02

		771		96.09

		770		96.14

		769		96.16

		768		96.16

		767		96.14

		766		96.1

		765		96.02

		764		95.9

		763		95.73

		762		95.52

		761		95.25

		760		94.95

		759		94.64

		758		94.32

		757		94.02

		756		93.75

		755		93.53

		754		93.39

		753		93.34

		752		93.39

		751		93.53

		750		93.75

		749		94

		748		94.28

		747		94.54

		746		94.77

		745		94.96

		744		95.09

		743		95.14

		742		95.1

		741		94.96

		740		94.7

		739		94.31

		738		93.79

		737		93.11

		736		92.28

		735		91.3

		734		90.21

		733		89.02

		732		87.74

		731		86.41

		730		85.07

		729		83.76

		728		82.56

		727		81.55

		726		80.77

		725		80.26

		724		80.01

		723		80

		722		80.25

		721		80.74

		720		81.49

		719		82.46

		718		83.61

		717		84.85

		716		86.12

		715		87.36

		714		88.53

		713		89.62

		712		90.61

		711		91.47

		710		92.18

		709		92.74

		708		93.14

		707		93.42

		706		93.58

		705		93.65

		704		93.64

		703		93.55

		702		93.39

		701		93.16

		700		92.84

		699		92.45

		698		91.97

		697		91.42

		696		90.8

		695		90.13

		694		89.43

		693		88.72

		692		88.04

		691		87.41

		690		86.86

		689		86.41

		688		86.07

		687		85.87

		686		85.79

		685		85.82

		684		85.97

		683		86.2

		682		86.49

		681		86.83

		680		87.19

		679		87.55

		678		87.91

		677		88.25

		676		88.56

		675		88.85

		674		89.13

		673		89.38

		672		89.63

		671		89.87

		670		90.12

		669		90.37

		668		90.63

		667		90.89

		666		91.16

		665		91.44

		664		91.73

		663		92.02

		662		92.31

		661		92.6

		660		92.88

		659		93.15

		658		93.41

		657		93.66

		656		93.89

		655		94.11

		654		94.31

		653		94.49

		652		94.65

		651		94.8

		650		94.92

		649		95.03

		648		95.12

		647		95.19

		646		95.25

		645		95.29

		644		95.33

		643		95.35

		642		95.37

		641		95.38

		640		95.4

		639		95.41

		638		95.43

		637		95.46

		636		95.49

		635		95.53

		634		95.58

		633		95.63

		632		95.68

		631		95.74

		630		95.8

		629		95.86

		628		95.92

		627		95.98

		626		96.04

		625		96.09

		624		96.14

		623		96.19

		622		96.23

		621		96.27

		620		96.31

		619		96.34

		618		96.37

		617		96.4

		616		96.42

		615		96.44

		614		96.45

		613		96.46

		612		96.48

		611		96.48

		610		96.49

		609		96.5

		608		96.51

		607		96.52

		606		96.53

		605		96.55

		604		96.56

		603		96.57

		602		96.58

		601		96.6

		600		96.61

		599		96.62

		598		96.63

		597		96.64

		596		96.64

		595		96.65

		594		96.65

		593		96.65

		592		96.65

		591		96.65

		590		96.64

		589		96.63

		588		96.62

		587		96.61

		586		96.59

		585		96.56

		584		96.53

		583		96.49

		582		96.44

		581		96.38

		580		96.32

		579		96.24

		578		96.15

		577		96.04

		576		95.92

		575		95.79

		574		95.63

		573		95.46

		572		95.26

		571		95.05

		570		94.81

		569		94.56

		568		94.27

		567		93.97

		566		93.64

		565		93.29

		564		92.91

		563		92.51

		562		92.08

		561		91.63

		560		91.16

		559		90.67

		558		90.17

		557		89.66

		556		89.15

		555		88.66

		554		88.2

		553		87.78

		552		87.42

		551		87.13

		550		86.93

		549		86.83

		548		86.84

		547		86.96

		546		87.2

		545		87.55

		544		87.99

		543		88.52

		542		89.12

		541		89.76

		540		90.42

		539		91.09

		538		91.74

		537		92.36

		536		92.93

		535		93.44

		534		93.9

		533		94.3

		532		94.64

		531		94.93

		530		95.18

		529		95.39

		528		95.57

		527		95.71

		526		95.84

		525		95.95

		524		96.05

		523		96.14

		522		96.22

		521		96.29

		520		96.34

		519		96.38

		518		96.42

		517		96.44

		516		96.45

		515		96.43

		514		96.4

		513		96.32

		512		96.21

		511		96.03

		510		95.79

		509		95.48

		508		95.1

		507		94.66

		506		94.17

		505		93.65

		504		93.12

		503		92.61

		502		92.16

		501		91.8

		500		91.55

		499		91.43

		498		91.45

		497		91.59

		496		91.84

		495		92.19

		494		92.59

		493		93.03

		492		93.47

		491		93.9

		490		94.29

		489		94.62

		488		94.9

		487		95.13

		486		95.3

		485		95.44

		484		95.55

		483		95.64

		482		95.72

		481		95.79

		480		95.86

		479		95.94

		478		96.02

		477		96.1

		476		96.18

		475		96.26

		474		96.33

		473		96.4

		472		96.46

		471		96.51

		470		96.54

		469		96.57

		468		96.58

		467		96.58

		466		96.58

		465		96.58

		464		96.57

		463		96.58

		462		96.58

		461		96.58

		460		96.58

		459		96.58

		458		96.58

		457		96.57

		456		96.55

		455		96.52

		454		96.46

		453		96.38

		452		96.28

		451		96.14

		450		95.97

		449		95.75

		448		95.46

		447		95.11

		446		94.68

		445		94.18

		444		93.62

		443		93.01

		442		92.38

		441		91.75

		440		91.16

		439		90.65

		438		90.24

		437		89.97

		436		89.86

		435		89.93

		434		90.16

		433		90.54

		432		91.04

		431		91.62

		430		92.26

		429		92.9

		428		93.53

		427		94.11

		426		94.6

		425		95

		424		95.3

		423		95.49

		422		95.59

		421		95.63

		420		95.61

		419		95.55

		418		95.48

		417		95.41

		416		95.36

		415		95.34

		414		95.37

		413		95.43

		412		95.54

		411		95.68

		410		95.84

		409		96.01

		408		96.17

		407		96.32

		406		96.45

		405		96.56

		404		96.64

		403		96.7

		402		96.73

		401		96.75

		400		96.76
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		cm-1		%T

		4000		95.17

		3999		95.17

		3998		95.17

		3997		95.17

		3996		95.17

		3995		95.17

		3994		95.17

		3993		95.17

		3992		95.17

		3991		95.17

		3990		95.17

		3989		95.16

		3988		95.16

		3987		95.16

		3986		95.16

		3985		95.16

		3984		95.16

		3983		95.16

		3982		95.15

		3981		95.15

		3980		95.15

		3979		95.16

		3978		95.16

		3977		95.16

		3976		95.16

		3975		95.16

		3974		95.16

		3973		95.16

		3972		95.16

		3971		95.16

		3970		95.16

		3969		95.16

		3968		95.16

		3967		95.16

		3966		95.16

		3965		95.16

		3964		95.16

		3963		95.16

		3962		95.16

		3961		95.16

		3960		95.16

		3959		95.16

		3958		95.16

		3957		95.16

		3956		95.16

		3955		95.16

		3954		95.16

		3953		95.16

		3952		95.16

		3951		95.16

		3950		95.15

		3949		95.15

		3948		95.15

		3947		95.15

		3946		95.15

		3945		95.15

		3944		95.15

		3943		95.15

		3942		95.15

		3941		95.15

		3940		95.15

		3939		95.15

		3938		95.15

		3937		95.15

		3936		95.15

		3935		95.15

		3934		95.15

		3933		95.15

		3932		95.16

		3931		95.16

		3930		95.16

		3929		95.16

		3928		95.16

		3927		95.16

		3926		95.16

		3925		95.15

		3924		95.15

		3923		95.15

		3922		95.14

		3921		95.14

		3920		95.13

		3919		95.13

		3918		95.12

		3917		95.12

		3916		95.12

		3915		95.12

		3914		95.12

		3913		95.12

		3912		95.12

		3911		95.12

		3910		95.12

		3909		95.12

		3908		95.12

		3907		95.12

		3906		95.12

		3905		95.12

		3904		95.11

		3903		95.11

		3902		95.11

		3901		95.11

		3900		95.12

		3899		95.12

		3898		95.12

		3897		95.12

		3896		95.12

		3895		95.12

		3894		95.12

		3893		95.11

		3892		95.11

		3891		95.11

		3890		95.11

		3889		95.11

		3888		95.1

		3887		95.1

		3886		95.1

		3885		95.1

		3884		95.1

		3883		95.1

		3882		95.1

		3881		95.11

		3880		95.11

		3879		95.11

		3878		95.11

		3877		95.11

		3876		95.11

		3875		95.1

		3874		95.1

		3873		95.1

		3872		95.1

		3871		95.1

		3870		95.1

		3869		95.1

		3868		95.1

		3867		95.1

		3866		95.1

		3865		95.1

		3864		95.1

		3863		95.1

		3862		95.1

		3861		95.1

		3860		95.1

		3859		95.1

		3858		95.1

		3857		95.1

		3856		95.1

		3855		95.1

		3854		95.1

		3853		95.1

		3852		95.1

		3851		95.1

		3850		95.1

		3849		95.1

		3848		95.1

		3847		95.1

		3846		95.1

		3845		95.1

		3844		95.1

		3843		95.1

		3842		95.1

		3841		95.09

		3840		95.09

		3839		95.09

		3838		95.09

		3837		95.09

		3836		95.09

		3835		95.09

		3834		95.09

		3833		95.09

		3832		95.09

		3831		95.09

		3830		95.09

		3829		95.09

		3828		95.1

		3827		95.1

		3826		95.1

		3825		95.1

		3824		95.1

		3823		95.1

		3822		95.1

		3821		95.1

		3820		95.1

		3819		95.1

		3818		95.11

		3817		95.11

		3816		95.11

		3815		95.11

		3814		95.11

		3813		95.11

		3812		95.11

		3811		95.11

		3810		95.11

		3809		95.11

		3808		95.1

		3807		95.1

		3806		95.1

		3805		95.1

		3804		95.1

		3803		95.11

		3802		95.11

		3801		95.11

		3800		95.11

		3799		95.12

		3798		95.12

		3797		95.12

		3796		95.12

		3795		95.13

		3794		95.13

		3793		95.13

		3792		95.13

		3791		95.14

		3790		95.14

		3789		95.14

		3788		95.14

		3787		95.15

		3786		95.15

		3785		95.15

		3784		95.15

		3783		95.16

		3782		95.16

		3781		95.16

		3780		95.16

		3779		95.16

		3778		95.16

		3777		95.16

		3776		95.16

		3775		95.16

		3774		95.16

		3773		95.15

		3772		95.15

		3771		95.15

		3770		95.15

		3769		95.15

		3768		95.15

		3767		95.14

		3766		95.14

		3765		95.14

		3764		95.14

		3763		95.14

		3762		95.14

		3761		95.13

		3760		95.13

		3759		95.12

		3758		95.12

		3757		95.11

		3756		95.1

		3755		95.09

		3754		95.08

		3753		95.07

		3752		95.07

		3751		95.06

		3750		95.06

		3749		95.05

		3748		95.05

		3747		95.06

		3746		95.06

		3745		95.06

		3744		95.07

		3743		95.07

		3742		95.08

		3741		95.09

		3740		95.09

		3739		95.1

		3738		95.1

		3737		95.1

		3736		95.11

		3735		95.11

		3734		95.11

		3733		95.11

		3732		95.11

		3731		95.11

		3730		95.11

		3729		95.11

		3728		95.11

		3727		95.11

		3726		95.11

		3725		95.11

		3724		95.1

		3723		95.1

		3722		95.09

		3721		95.09

		3720		95.08

		3719		95.07

		3718		95.06

		3717		95.05

		3716		95.04

		3715		95.03

		3714		95.02

		3713		95.01

		3712		95

		3711		94.99

		3710		94.98

		3709		94.98

		3708		94.97

		3707		94.97

		3706		94.96

		3705		94.95

		3704		94.94

		3703		94.94

		3702		94.93

		3701		94.91

		3700		94.9

		3699		94.89

		3698		94.87

		3697		94.86

		3696		94.84

		3695		94.83

		3694		94.82

		3693		94.8

		3692		94.79

		3691		94.78

		3690		94.77

		3689		94.76

		3688		94.74

		3687		94.73

		3686		94.72

		3685		94.71

		3684		94.7

		3683		94.69

		3682		94.67

		3681		94.66

		3680		94.65

		3679		94.64

		3678		94.63

		3677		94.62

		3676		94.61

		3675		94.61

		3674		94.61

		3673		94.6

		3672		94.6

		3671		94.6

		3670		94.6

		3669		94.61

		3668		94.61

		3667		94.61

		3666		94.61

		3665		94.61

		3664		94.61

		3663		94.62

		3662		94.62

		3661		94.63

		3660		94.63

		3659		94.64

		3658		94.65

		3657		94.66

		3656		94.67

		3655		94.68

		3654		94.69

		3653		94.71

		3652		94.72

		3651		94.74

		3650		94.75

		3649		94.77

		3648		94.79

		3647		94.81

		3646		94.82

		3645		94.84

		3644		94.86

		3643		94.87

		3642		94.89

		3641		94.9

		3640		94.92

		3639		94.93

		3638		94.94

		3637		94.96

		3636		94.97

		3635		94.97

		3634		94.98

		3633		94.99

		3632		95

		3631		95

		3630		95.01

		3629		95.02

		3628		95.03

		3627		95.04

		3626		95.05

		3625		95.06

		3624		95.07

		3623		95.08

		3622		95.08

		3621		95.09

		3620		95.09

		3619		95.09

		3618		95.09

		3617		95.08

		3616		95.07

		3615		95.07

		3614		95.06

		3613		95.05

		3612		95.04

		3611		95.04

		3610		95.03

		3609		95.03

		3608		95.03

		3607		95.04

		3606		95.04

		3605		95.05

		3604		95.05

		3603		95.06

		3602		95.07

		3601		95.08

		3600		95.09

		3599		95.1

		3598		95.1

		3597		95.11

		3596		95.12

		3595		95.12

		3594		95.13

		3593		95.13

		3592		95.13

		3591		95.14

		3590		95.14

		3589		95.15

		3588		95.15

		3587		95.15

		3586		95.16

		3585		95.16

		3584		95.16

		3583		95.17

		3582		95.17

		3581		95.17

		3580		95.17

		3579		95.17

		3578		95.17

		3577		95.17

		3576		95.17

		3575		95.17

		3574		95.17

		3573		95.17

		3572		95.17

		3571		95.17

		3570		95.17

		3569		95.17

		3568		95.17

		3567		95.17

		3566		95.17

		3565		95.17

		3564		95.17

		3563		95.17

		3562		95.17

		3561		95.17

		3560		95.17

		3559		95.17

		3558		95.17

		3557		95.17

		3556		95.17

		3555		95.17

		3554		95.17

		3553		95.17

		3552		95.17

		3551		95.16

		3550		95.16

		3549		95.16

		3548		95.16

		3547		95.16

		3546		95.16

		3545		95.15

		3544		95.15

		3543		95.15

		3542		95.15

		3541		95.15

		3540		95.15

		3539		95.15

		3538		95.15

		3537		95.15

		3536		95.16

		3535		95.16

		3534		95.16

		3533		95.16

		3532		95.16

		3531		95.16

		3530		95.16

		3529		95.16

		3528		95.16

		3527		95.16

		3526		95.16

		3525		95.16

		3524		95.16

		3523		95.16

		3522		95.16

		3521		95.16

		3520		95.16

		3519		95.17

		3518		95.17

		3517		95.17

		3516		95.17

		3515		95.17

		3514		95.17

		3513		95.17

		3512		95.17

		3511		95.17

		3510		95.17

		3509		95.17

		3508		95.17

		3507		95.17

		3506		95.17

		3505		95.16

		3504		95.16

		3503		95.16

		3502		95.16

		3501		95.16

		3500		95.16

		3499		95.16

		3498		95.16

		3497		95.16

		3496		95.16

		3495		95.16

		3494		95.16

		3493		95.17

		3492		95.17

		3491		95.17

		3490		95.17

		3489		95.17

		3488		95.17

		3487		95.17

		3486		95.17

		3485		95.17

		3484		95.17

		3483		95.17

		3482		95.16

		3481		95.16

		3480		95.16

		3479		95.16

		3478		95.16

		3477		95.16

		3476		95.16

		3475		95.16

		3474		95.16

		3473		95.16

		3472		95.16

		3471		95.16

		3470		95.17

		3469		95.17

		3468		95.17

		3467		95.17

		3466		95.17

		3465		95.17

		3464		95.17

		3463		95.16

		3462		95.16

		3461		95.16

		3460		95.16

		3459		95.16

		3458		95.15

		3457		95.15

		3456		95.15

		3455		95.15

		3454		95.15

		3453		95.15

		3452		95.14

		3451		95.14

		3450		95.14

		3449		95.14

		3448		95.14

		3447		95.14

		3446		95.14

		3445		95.14

		3444		95.14

		3443		95.14

		3442		95.14

		3441		95.14

		3440		95.14

		3439		95.14

		3438		95.14

		3437		95.14

		3436		95.13

		3435		95.13

		3434		95.12

		3433		95.12

		3432		95.11

		3431		95.1

		3430		95.09

		3429		95.08

		3428		95.08

		3427		95.07

		3426		95.06

		3425		95.05

		3424		95.04

		3423		95.04

		3422		95.03

		3421		95.02

		3420		95.02

		3419		95.02

		3418		95.02

		3417		95.01

		3416		95.01

		3415		95.01

		3414		95.01

		3413		95.01

		3412		95.01

		3411		95.01

		3410		95.01

		3409		95.01

		3408		95.01

		3407		95.01

		3406		95.01

		3405		95.01

		3404		95.01

		3403		95.01

		3402		95.02

		3401		95.02

		3400		95.02

		3399		95.01

		3398		95.01

		3397		95.01

		3396		95

		3395		95

		3394		94.99

		3393		94.98

		3392		94.97

		3391		94.96

		3390		94.95

		3389		94.94

		3388		94.93

		3387		94.92

		3386		94.91

		3385		94.9

		3384		94.9

		3383		94.9

		3382		94.9

		3381		94.9

		3380		94.9

		3379		94.91

		3378		94.91

		3377		94.92

		3376		94.93

		3375		94.93

		3374		94.94

		3373		94.95

		3372		94.95

		3371		94.96

		3370		94.96

		3369		94.96

		3368		94.96

		3367		94.95

		3366		94.94

		3365		94.94

		3364		94.93

		3363		94.92

		3362		94.91

		3361		94.9

		3360		94.89

		3359		94.89

		3358		94.88

		3357		94.88

		3356		94.88

		3355		94.88

		3354		94.88

		3353		94.88

		3352		94.88

		3351		94.88

		3350		94.88

		3349		94.87

		3348		94.87

		3347		94.87

		3346		94.86

		3345		94.86

		3344		94.85

		3343		94.85

		3342		94.84

		3341		94.83

		3340		94.83

		3339		94.82

		3338		94.82

		3337		94.81

		3336		94.81

		3335		94.8

		3334		94.8

		3333		94.79

		3332		94.79

		3331		94.78

		3330		94.78

		3329		94.78

		3328		94.77

		3327		94.77

		3326		94.77

		3325		94.76

		3324		94.76

		3323		94.76

		3322		94.76

		3321		94.75

		3320		94.75

		3319		94.75

		3318		94.75

		3317		94.75

		3316		94.75

		3315		94.76

		3314		94.76

		3313		94.76

		3312		94.76

		3311		94.76

		3310		94.76

		3309		94.76

		3308		94.76

		3307		94.76

		3306		94.76

		3305		94.75

		3304		94.75

		3303		94.74

		3302		94.74

		3301		94.73

		3300		94.73

		3299		94.72

		3298		94.71

		3297		94.71

		3296		94.7

		3295		94.69

		3294		94.69

		3293		94.68

		3292		94.67

		3291		94.66

		3290		94.65

		3289		94.64

		3288		94.63

		3287		94.62

		3286		94.62

		3285		94.61

		3284		94.6

		3283		94.59

		3282		94.59

		3281		94.58

		3280		94.57

		3279		94.57

		3278		94.56

		3277		94.55

		3276		94.55

		3275		94.54

		3274		94.53

		3273		94.53

		3272		94.52

		3271		94.51

		3270		94.5

		3269		94.49

		3268		94.48

		3267		94.47

		3266		94.46

		3265		94.44

		3264		94.43

		3263		94.42

		3262		94.41

		3261		94.4

		3260		94.39

		3259		94.38

		3258		94.37

		3257		94.36

		3256		94.35

		3255		94.34

		3254		94.33

		3253		94.32

		3252		94.31

		3251		94.3

		3250		94.29

		3249		94.28

		3248		94.26

		3247		94.25

		3246		94.24

		3245		94.23

		3244		94.21

		3243		94.2

		3242		94.19

		3241		94.17

		3240		94.16

		3239		94.15

		3238		94.13

		3237		94.12

		3236		94.1

		3235		94.09

		3234		94.08

		3233		94.06

		3232		94.05

		3231		94.04

		3230		94.02

		3229		94.01

		3228		93.99

		3227		93.98

		3226		93.97

		3225		93.95

		3224		93.94

		3223		93.92

		3222		93.91

		3221		93.89

		3220		93.87

		3219		93.86

		3218		93.84

		3217		93.83

		3216		93.81

		3215		93.8

		3214		93.78

		3213		93.77

		3212		93.75

		3211		93.74

		3210		93.72

		3209		93.71

		3208		93.69

		3207		93.68

		3206		93.66

		3205		93.65

		3204		93.64

		3203		93.62

		3202		93.61

		3201		93.59

		3200		93.58

		3199		93.56

		3198		93.55

		3197		93.54

		3196		93.52

		3195		93.51

		3194		93.5

		3193		93.48

		3192		93.47

		3191		93.46

		3190		93.44

		3189		93.43

		3188		93.41

		3187		93.4

		3186		93.38

		3185		93.37

		3184		93.35

		3183		93.34

		3182		93.32

		3181		93.31

		3180		93.29

		3179		93.28

		3178		93.27

		3177		93.25

		3176		93.24

		3175		93.23

		3174		93.21

		3173		93.2

		3172		93.19

		3171		93.17

		3170		93.16

		3169		93.14

		3168		93.12

		3167		93.11

		3166		93.09

		3165		93.07

		3164		93.06

		3163		93.04

		3162		93.02

		3161		93.01

		3160		92.99

		3159		92.97

		3158		92.95

		3157		92.93

		3156		92.91

		3155		92.89

		3154		92.87

		3153		92.85

		3152		92.83

		3151		92.81

		3150		92.79

		3149		92.76

		3148		92.74

		3147		92.72

		3146		92.7

		3145		92.67

		3144		92.65

		3143		92.62

		3142		92.6

		3141		92.57

		3140		92.55

		3139		92.52

		3138		92.5

		3137		92.47

		3136		92.44

		3135		92.42

		3134		92.39

		3133		92.36

		3132		92.33

		3131		92.31

		3130		92.28

		3129		92.25

		3128		92.23

		3127		92.2

		3126		92.17

		3125		92.14

		3124		92.11

		3123		92.08

		3122		92.06

		3121		92.03

		3120		92

		3119		91.97

		3118		91.94

		3117		91.91

		3116		91.88

		3115		91.85

		3114		91.82

		3113		91.79

		3112		91.76

		3111		91.73

		3110		91.7

		3109		91.67

		3108		91.64

		3107		91.61

		3106		91.58

		3105		91.55

		3104		91.52

		3103		91.49

		3102		91.46

		3101		91.44

		3100		91.41

		3099		91.38

		3098		91.36

		3097		91.33

		3096		91.31

		3095		91.29

		3094		91.27

		3093		91.24

		3092		91.22

		3091		91.2

		3090		91.18

		3089		91.16

		3088		91.14

		3087		91.12

		3086		91.11

		3085		91.09

		3084		91.07

		3083		91.05

		3082		91.03

		3081		91.01

		3080		90.99

		3079		90.97

		3078		90.94

		3077		90.92

		3076		90.9

		3075		90.88

		3074		90.86

		3073		90.84

		3072		90.81

		3071		90.79

		3070		90.77

		3069		90.75

		3068		90.72

		3067		90.7

		3066		90.68

		3065		90.65

		3064		90.63

		3063		90.6

		3062		90.58

		3061		90.55

		3060		90.53

		3059		90.5

		3058		90.47

		3057		90.44

		3056		90.41

		3055		90.38

		3054		90.34

		3053		90.31

		3052		90.27

		3051		90.23

		3050		90.19

		3049		90.15

		3048		90.11

		3047		90.07

		3046		90.02

		3045		89.98

		3044		89.93

		3043		89.88

		3042		89.83

		3041		89.78

		3040		89.73

		3039		89.67

		3038		89.62

		3037		89.56

		3036		89.51

		3035		89.45

		3034		89.39

		3033		89.33

		3032		89.27

		3031		89.22

		3030		89.16

		3029		89.1

		3028		89.04

		3027		88.99

		3026		88.93

		3025		88.88

		3024		88.82

		3023		88.77

		3022		88.71

		3021		88.66

		3020		88.6

		3019		88.55

		3018		88.5

		3017		88.45

		3016		88.4

		3015		88.35

		3014		88.3

		3013		88.25

		3012		88.2

		3011		88.16

		3010		88.12

		3009		88.07

		3008		88.04

		3007		88

		3006		87.96

		3005		87.93

		3004		87.89

		3003		87.86

		3002		87.83

		3001		87.8

		3000		87.77

		2999		87.74

		2998		87.7

		2997		87.67

		2996		87.63

		2995		87.59

		2994		87.55

		2993		87.5

		2992		87.45

		2991		87.4

		2990		87.36

		2989		87.31

		2988		87.26

		2987		87.22

		2986		87.17

		2985		87.13

		2984		87.08

		2983		87.03

		2982		86.98

		2981		86.91

		2980		86.84

		2979		86.75

		2978		86.64

		2977		86.51

		2976		86.33

		2975		86.11

		2974		85.83

		2973		85.49

		2972		85.1

		2971		84.65

		2970		84.15

		2969		83.62

		2968		83.06

		2967		82.48

		2966		81.89

		2965		81.31

		2964		80.75

		2963		80.22

		2962		79.73

		2961		79.28

		2960		78.89

		2959		78.55

		2958		78.28

		2957		78.07

		2956		77.93

		2955		77.87

		2954		77.89

		2953		77.98

		2952		78.14

		2951		78.33

		2950		78.55

		2949		78.76

		2948		78.95

		2947		79.09

		2946		79.17

		2945		79.17

		2944		79.08

		2943		78.91

		2942		78.67

		2941		78.35

		2940		77.98

		2939		77.58

		2938		77.15

		2937		76.72

		2936		76.28

		2935		75.84

		2934		75.38

		2933		74.91

		2932		74.39

		2931		73.82

		2930		73.16

		2929		72.4

		2928		71.51

		2927		70.47

		2926		69.27

		2925		67.91

		2924		66.4

		2923		64.77

		2922		63.07

		2921		61.33

		2920		59.64

		2919		58.06

		2918		56.66

		2917		55.51

		2916		54.67

		2915		54.16

		2914		54.02

		2913		54.25

		2912		54.81

		2911		55.66

		2910		56.76

		2909		58.02

		2908		59.4

		2907		60.83

		2906		62.25

		2905		63.62

		2904		64.91

		2903		66.09

		2902		67.17

		2901		68.13

		2900		69

		2899		69.77

		2898		70.48

		2897		71.12

		2896		71.72

		2895		72.28

		2894		72.82

		2893		73.33

		2892		73.84

		2891		74.33

		2890		74.82

		2889		75.31

		2888		75.79

		2887		76.26

		2886		76.72

		2885		77.15

		2884		77.55

		2883		77.9

		2882		78.2

		2881		78.44

		2880		78.61

		2879		78.72

		2878		78.77

		2877		78.77

		2876		78.73

		2875		78.67

		2874		78.6

		2873		78.55

		2872		78.51

		2871		78.5

		2870		78.52

		2869		78.55

		2868		78.6

		2867		78.62

		2866		78.62

		2865		78.55

		2864		78.4

		2863		78.13

		2862		77.72

		2861		77.13

		2860		76.35

		2859		75.35

		2858		74.15

		2857		72.75

		2856		71.2

		2855		69.54

		2854		67.85

		2853		66.19

		2852		64.64

		2851		63.31

		2850		62.26

		2849		61.59

		2848		61.33

		2847		61.51

		2846		62.11

		2845		63.09

		2844		64.38

		2843		65.92

		2842		67.61

		2841		69.38

		2840		71.15

		2839		72.86

		2838		74.45

		2837		75.89

		2836		77.16

		2835		78.27

		2834		79.23

		2833		80.05

		2832		80.76

		2831		81.38

		2830		81.91

		2829		82.38

		2828		82.8

		2827		83.17

		2826		83.5

		2825		83.8

		2824		84.07

		2823		84.31

		2822		84.54

		2821		84.75

		2820		84.94

		2819		85.12

		2818		85.29

		2817		85.45

		2816		85.59

		2815		85.73

		2814		85.85

		2813		85.97

		2812		86.09

		2811		86.2

		2810		86.3

		2809		86.4

		2808		86.49

		2807		86.58

		2806		86.67

		2805		86.75

		2804		86.83

		2803		86.91

		2802		86.99

		2801		87.07

		2800		87.14

		2799		87.21

		2798		87.28

		2797		87.34

		2796		87.4

		2795		87.46

		2794		87.52

		2793		87.57

		2792		87.62

		2791		87.67

		2790		87.71

		2789		87.75

		2788		87.79

		2787		87.83

		2786		87.87

		2785		87.9

		2784		87.93

		2783		87.96

		2782		87.99

		2781		88.02

		2780		88.04

		2779		88.07

		2778		88.09

		2777		88.12

		2776		88.14

		2775		88.16

		2774		88.18

		2773		88.2

		2772		88.22

		2771		88.25

		2770		88.27

		2769		88.29

		2768		88.31

		2767		88.33

		2766		88.36

		2765		88.38

		2764		88.4

		2763		88.43

		2762		88.45

		2761		88.47

		2760		88.5

		2759		88.52

		2758		88.54

		2757		88.56

		2756		88.59

		2755		88.61

		2754		88.63

		2753		88.65

		2752		88.67

		2751		88.69

		2750		88.72

		2749		88.74

		2748		88.76

		2747		88.78

		2746		88.81

		2745		88.83

		2744		88.85

		2743		88.87

		2742		88.89

		2741		88.91

		2740		88.93

		2739		88.95

		2738		88.97

		2737		88.98

		2736		89

		2735		89.01

		2734		89.02

		2733		89.04

		2732		89.05

		2731		89.06

		2730		89.07

		2729		89.08

		2728		89.1

		2727		89.11

		2726		89.12

		2725		89.13

		2724		89.14

		2723		89.15

		2722		89.15

		2721		89.15

		2720		89.14

		2719		89.14

		2718		89.12

		2717		89.11

		2716		89.09

		2715		89.06

		2714		89.04

		2713		89.01

		2712		88.98

		2711		88.95

		2710		88.92

		2709		88.89

		2708		88.86

		2707		88.83

		2706		88.81

		2705		88.78

		2704		88.76

		2703		88.74

		2702		88.72

		2701		88.71

		2700		88.69

		2699		88.67

		2698		88.65

		2697		88.64

		2696		88.62

		2695		88.6

		2694		88.58

		2693		88.55

		2692		88.53

		2691		88.51

		2690		88.48

		2689		88.46

		2688		88.44

		2687		88.42

		2686		88.4

		2685		88.38

		2684		88.37

		2683		88.35

		2682		88.34

		2681		88.33

		2680		88.33

		2679		88.32

		2678		88.32

		2677		88.32

		2676		88.32

		2675		88.32

		2674		88.32

		2673		88.32

		2672		88.32

		2671		88.32

		2670		88.33

		2669		88.33

		2668		88.33

		2667		88.33

		2666		88.33

		2665		88.34

		2664		88.34

		2663		88.34

		2662		88.34

		2661		88.34

		2660		88.34

		2659		88.34

		2658		88.34

		2657		88.34

		2656		88.34

		2655		88.34

		2654		88.34

		2653		88.34

		2652		88.34

		2651		88.34

		2650		88.35

		2649		88.36

		2648		88.37

		2647		88.38

		2646		88.39

		2645		88.4

		2644		88.41

		2643		88.43

		2642		88.44

		2641		88.45

		2640		88.46

		2639		88.47

		2638		88.48

		2637		88.49

		2636		88.49

		2635		88.5

		2634		88.51

		2633		88.51

		2632		88.52

		2631		88.53

		2630		88.54

		2629		88.56

		2628		88.58

		2627		88.6

		2626		88.62

		2625		88.65

		2624		88.67

		2623		88.7

		2622		88.73

		2621		88.76

		2620		88.78

		2619		88.81

		2618		88.83

		2617		88.86

		2616		88.88

		2615		88.89

		2614		88.91

		2613		88.92

		2612		88.94

		2611		88.95

		2610		88.96

		2609		88.98

		2608		88.99

		2607		89.01

		2606		89.02

		2605		89.04

		2604		89.06

		2603		89.09

		2602		89.11

		2601		89.14

		2600		89.16

		2599		89.19

		2598		89.22

		2597		89.25

		2596		89.28

		2595		89.31

		2594		89.34

		2593		89.37

		2592		89.39

		2591		89.42

		2590		89.44

		2589		89.47

		2588		89.49

		2587		89.51

		2586		89.52

		2585		89.54

		2584		89.55

		2583		89.56

		2582		89.58

		2581		89.59

		2580		89.6

		2579		89.61

		2578		89.62

		2577		89.63

		2576		89.63

		2575		89.64

		2574		89.65

		2573		89.66

		2572		89.66

		2571		89.67

		2570		89.67

		2569		89.67

		2568		89.67

		2567		89.67

		2566		89.67

		2565		89.67

		2564		89.67

		2563		89.67

		2562		89.68

		2561		89.68

		2560		89.69

		2559		89.7

		2558		89.72

		2557		89.73

		2556		89.76

		2555		89.78

		2554		89.81

		2553		89.84

		2552		89.87

		2551		89.91

		2550		89.94

		2549		89.98

		2548		90.02

		2547		90.05

		2546		90.08

		2545		90.12

		2544		90.15

		2543		90.17

		2542		90.19

		2541		90.21

		2540		90.23

		2539		90.24

		2538		90.25

		2537		90.26

		2536		90.28

		2535		90.29

		2534		90.3

		2533		90.32

		2532		90.34

		2531		90.37

		2530		90.4

		2529		90.44

		2528		90.49

		2527		90.54

		2526		90.59

		2525		90.64

		2524		90.7

		2523		90.75

		2522		90.8

		2521		90.85

		2520		90.9

		2519		90.94

		2518		90.97

		2517		91.01

		2516		91.04

		2515		91.07

		2514		91.1

		2513		91.12

		2512		91.15

		2511		91.18

		2510		91.21

		2509		91.24

		2508		91.28

		2507		91.32

		2506		91.36

		2505		91.4

		2504		91.44

		2503		91.48

		2502		91.52

		2501		91.56

		2500		91.59

		2499		91.63

		2498		91.65

		2497		91.68

		2496		91.7

		2495		91.72

		2494		91.74

		2493		91.75

		2492		91.76

		2491		91.78

		2490		91.79

		2489		91.81

		2488		91.83

		2487		91.85

		2486		91.87

		2485		91.9

		2484		91.93

		2483		91.96

		2482		91.99

		2481		92.02

		2480		92.06

		2479		92.09

		2478		92.12

		2477		92.15

		2476		92.17

		2475		92.19

		2474		92.21

		2473		92.23

		2472		92.25

		2471		92.26

		2470		92.27

		2469		92.28

		2468		92.29

		2467		92.3

		2466		92.32

		2465		92.33

		2464		92.35

		2463		92.36

		2462		92.38

		2461		92.4

		2460		92.43

		2459		92.45

		2458		92.47

		2457		92.5

		2456		92.52

		2455		92.54

		2454		92.57

		2453		92.59

		2452		92.6

		2451		92.62

		2450		92.64

		2449		92.65

		2448		92.66

		2447		92.67

		2446		92.68

		2445		92.7

		2444		92.71

		2443		92.72

		2442		92.73

		2441		92.75

		2440		92.77

		2439		92.79

		2438		92.81

		2437		92.83

		2436		92.85

		2435		92.88

		2434		92.9

		2433		92.92

		2432		92.94

		2431		92.96

		2430		92.98

		2429		93

		2428		93.01

		2427		93.03

		2426		93.04

		2425		93.05

		2424		93.05

		2423		93.06

		2422		93.07

		2421		93.08

		2420		93.08

		2419		93.09

		2418		93.1

		2417		93.11

		2416		93.12

		2415		93.14

		2414		93.15

		2413		93.17

		2412		93.18

		2411		93.2

		2410		93.22

		2409		93.23

		2408		93.25

		2407		93.26

		2406		93.28

		2405		93.29

		2404		93.3

		2403		93.31

		2402		93.32

		2401		93.33

		2400		93.34

		2399		93.35

		2398		93.36

		2397		93.36

		2396		93.37

		2395		93.38

		2394		93.39

		2393		93.4

		2392		93.41

		2391		93.42

		2390		93.43

		2389		93.45

		2388		93.46

		2387		93.47

		2386		93.49

		2385		93.5

		2384		93.52

		2383		93.53

		2382		93.54

		2381		93.55

		2380		93.56

		2379		93.56

		2378		93.57

		2377		93.57

		2376		93.58

		2375		93.58

		2374		93.59

		2373		93.59

		2372		93.6

		2371		93.61

		2370		93.61

		2369		93.62

		2368		93.62

		2367		93.62

		2366		93.62

		2365		93.62

		2364		93.62

		2363		93.62

		2362		93.62

		2361		93.62

		2360		93.62

		2359		93.63

		2358		93.63

		2357		93.63

		2356		93.64

		2355		93.64

		2354		93.65

		2353		93.65

		2352		93.65

		2351		93.65

		2350		93.65

		2349		93.65

		2348		93.65

		2347		93.65

		2346		93.64

		2345		93.64

		2344		93.64

		2343		93.64

		2342		93.64

		2341		93.64

		2340		93.64

		2339		93.65

		2338		93.65

		2337		93.66

		2336		93.66

		2335		93.66

		2334		93.65

		2333		93.65

		2332		93.64

		2331		93.63

		2330		93.62

		2329		93.61

		2328		93.6

		2327		93.59

		2326		93.58

		2325		93.57

		2324		93.57

		2323		93.58

		2322		93.58

		2321		93.59

		2320		93.6

		2319		93.62

		2318		93.64

		2317		93.65

		2316		93.67

		2315		93.69

		2314		93.71

		2313		93.73

		2312		93.74

		2311		93.76

		2310		93.78

		2309		93.79

		2308		93.81

		2307		93.82

		2306		93.83

		2305		93.84

		2304		93.85

		2303		93.85

		2302		93.86

		2301		93.86

		2300		93.86

		2299		93.86

		2298		93.86

		2297		93.86

		2296		93.86

		2295		93.85

		2294		93.85

		2293		93.84

		2292		93.84

		2291		93.84

		2290		93.83

		2289		93.83

		2288		93.83

		2287		93.83

		2286		93.83

		2285		93.84

		2284		93.84

		2283		93.85

		2282		93.86

		2281		93.87

		2280		93.88

		2279		93.89

		2278		93.9

		2277		93.92

		2276		93.93

		2275		93.94

		2274		93.96

		2273		93.98

		2272		93.99

		2271		94.01

		2270		94.02

		2269		94.04

		2268		94.05

		2267		94.06

		2266		94.08

		2265		94.09

		2264		94.1

		2263		94.1

		2262		94.11

		2261		94.12

		2260		94.13

		2259		94.14

		2258		94.15

		2257		94.17

		2256		94.18

		2255		94.2

		2254		94.22

		2253		94.23

		2252		94.25

		2251		94.26

		2250		94.27

		2249		94.29

		2248		94.3

		2247		94.31

		2246		94.31

		2245		94.32

		2244		94.33

		2243		94.34

		2242		94.34

		2241		94.35

		2240		94.36

		2239		94.37

		2238		94.38

		2237		94.39

		2236		94.39

		2235		94.4

		2234		94.41

		2233		94.42

		2232		94.43

		2231		94.44

		2230		94.45

		2229		94.46

		2228		94.47

		2227		94.48

		2226		94.49

		2225		94.5

		2224		94.51

		2223		94.52

		2222		94.53

		2221		94.53

		2220		94.54

		2219		94.54

		2218		94.55

		2217		94.54

		2216		94.54

		2215		94.54

		2214		94.53

		2213		94.52

		2212		94.52

		2211		94.52

		2210		94.51

		2209		94.51

		2208		94.52

		2207		94.52

		2206		94.52

		2205		94.53

		2204		94.53

		2203		94.54

		2202		94.54

		2201		94.55

		2200		94.55

		2199		94.54

		2198		94.54

		2197		94.53

		2196		94.53

		2195		94.52

		2194		94.52

		2193		94.52

		2192		94.52

		2191		94.52

		2190		94.53

		2189		94.54

		2188		94.55

		2187		94.57

		2186		94.59

		2185		94.61

		2184		94.63

		2183		94.65

		2182		94.67

		2181		94.68

		2180		94.69

		2179		94.7

		2178		94.7

		2177		94.69

		2176		94.69

		2175		94.67

		2174		94.66

		2173		94.65

		2172		94.63

		2171		94.61

		2170		94.6

		2169		94.59

		2168		94.59

		2167		94.6

		2166		94.62

		2165		94.64

		2164		94.68

		2163		94.72

		2162		94.76

		2161		94.82

		2160		94.87

		2159		94.92

		2158		94.97

		2157		95.01

		2156		95.04

		2155		95.06

		2154		95.07

		2153		95.08

		2152		95.08

		2151		95.07

		2150		95.06

		2149		95.05

		2148		95.04

		2147		95.03

		2146		95.02

		2145		95.01

		2144		95

		2143		94.99

		2142		94.99

		2141		94.99

		2140		94.99

		2139		94.99

		2138		94.99

		2137		94.99

		2136		94.98

		2135		94.98

		2134		94.98

		2133		94.98

		2132		94.97

		2131		94.96

		2130		94.95

		2129		94.94

		2128		94.93

		2127		94.91

		2126		94.9

		2125		94.88

		2124		94.87

		2123		94.85

		2122		94.84

		2121		94.83

		2120		94.81

		2119		94.8

		2118		94.79

		2117		94.77

		2116		94.77

		2115		94.76

		2114		94.76

		2113		94.76

		2112		94.76

		2111		94.76

		2110		94.77

		2109		94.77

		2108		94.77

		2107		94.77

		2106		94.78

		2105		94.78

		2104		94.78

		2103		94.78

		2102		94.78

		2101		94.78

		2100		94.78

		2099		94.79

		2098		94.79

		2097		94.79

		2096		94.79

		2095		94.8

		2094		94.8

		2093		94.8

		2092		94.8

		2091		94.8

		2090		94.79

		2089		94.79

		2088		94.78

		2087		94.78

		2086		94.77

		2085		94.77

		2084		94.76

		2083		94.76

		2082		94.76

		2081		94.76

		2080		94.76

		2079		94.77

		2078		94.78

		2077		94.78

		2076		94.79

		2075		94.8

		2074		94.81

		2073		94.82

		2072		94.83

		2071		94.83

		2070		94.84

		2069		94.84

		2068		94.85

		2067		94.85

		2066		94.85

		2065		94.86

		2064		94.86

		2063		94.86

		2062		94.87

		2061		94.87

		2060		94.87

		2059		94.87

		2058		94.87

		2057		94.87

		2056		94.86

		2055		94.86

		2054		94.86

		2053		94.86

		2052		94.86

		2051		94.86

		2050		94.87

		2049		94.88

		2048		94.88

		2047		94.89

		2046		94.9

		2045		94.91

		2044		94.91

		2043		94.91

		2042		94.92

		2041		94.92

		2040		94.93

		2039		94.94

		2038		94.95

		2037		94.96

		2036		94.97

		2035		94.99

		2034		95.01

		2033		95.03

		2032		95.04

		2031		95.06

		2030		95.07

		2029		95.08

		2028		95.08

		2027		95.09

		2026		95.09

		2025		95.09

		2024		95.08

		2023		95.08

		2022		95.07

		2021		95.07

		2020		95.06

		2019		95.06

		2018		95.06

		2017		95.07

		2016		95.07

		2015		95.08

		2014		95.09

		2013		95.1

		2012		95.11

		2011		95.12

		2010		95.13

		2009		95.14

		2008		95.14

		2007		95.15

		2006		95.14

		2005		95.14

		2004		95.12

		2003		95.11

		2002		95.1

		2001		95.08

		2000		95.06

		1999		95.05

		1998		95.03

		1997		95.02

		1996		95

		1995		94.99

		1994		94.98

		1993		94.97

		1992		94.95

		1991		94.94

		1990		94.92

		1989		94.91

		1988		94.89

		1987		94.88

		1986		94.87

		1985		94.87

		1984		94.87

		1983		94.88

		1982		94.89

		1981		94.91

		1980		94.93

		1979		94.96

		1978		94.99

		1977		95.03

		1976		95.06

		1975		95.08

		1974		95.11

		1973		95.13

		1972		95.14

		1971		95.15

		1970		95.16

		1969		95.16

		1968		95.15

		1967		95.15

		1966		95.15

		1965		95.15

		1964		95.14

		1963		95.14

		1962		95.13

		1961		95.13

		1960		95.12

		1959		95.12

		1958		95.11

		1957		95.09

		1956		95.08

		1955		95.07

		1954		95.06

		1953		95.04

		1952		95.03

		1951		95.02

		1950		95.02

		1949		95.02

		1948		95.01

		1947		95.02

		1946		95.02

		1945		95.03

		1944		95.03

		1943		95.03

		1942		95.04

		1941		95.04

		1940		95.04

		1939		95.04

		1938		95.04

		1937		95.03

		1936		95.03

		1935		95.02

		1934		95.02

		1933		95.01

		1932		95

		1931		95

		1930		94.99

		1929		94.98

		1928		94.97

		1927		94.96

		1926		94.95

		1925		94.94

		1924		94.93

		1923		94.92

		1922		94.91

		1921		94.9

		1920		94.89

		1919		94.88

		1918		94.87

		1917		94.87

		1916		94.87

		1915		94.86

		1914		94.86

		1913		94.86

		1912		94.86

		1911		94.86

		1910		94.85

		1909		94.85

		1908		94.84

		1907		94.84

		1906		94.83

		1905		94.82

		1904		94.8

		1903		94.79

		1902		94.78

		1901		94.77

		1900		94.76

		1899		94.75

		1898		94.75

		1897		94.75

		1896		94.74

		1895		94.74

		1894		94.75

		1893		94.75

		1892		94.75

		1891		94.75

		1890		94.75

		1889		94.75

		1888		94.74

		1887		94.74

		1886		94.73

		1885		94.73

		1884		94.72

		1883		94.72

		1882		94.71

		1881		94.7

		1880		94.7

		1879		94.69

		1878		94.68

		1877		94.68

		1876		94.67

		1875		94.67

		1874		94.66

		1873		94.65

		1872		94.64

		1871		94.63

		1870		94.63

		1869		94.62

		1868		94.61

		1867		94.6

		1866		94.59

		1865		94.58

		1864		94.57

		1863		94.56

		1862		94.55

		1861		94.54

		1860		94.53

		1859		94.52

		1858		94.51

		1857		94.49

		1856		94.48

		1855		94.47

		1854		94.45

		1853		94.44

		1852		94.42

		1851		94.41

		1850		94.4

		1849		94.39

		1848		94.38

		1847		94.37

		1846		94.36

		1845		94.36

		1844		94.35

		1843		94.34

		1842		94.33

		1841		94.33

		1840		94.32

		1839		94.31

		1838		94.3

		1837		94.29

		1836		94.29

		1835		94.28

		1834		94.27

		1833		94.26

		1832		94.25

		1831		94.23

		1830		94.22

		1829		94.21

		1828		94.19

		1827		94.17

		1826		94.15

		1825		94.13

		1824		94.11

		1823		94.09

		1822		94.07

		1821		94.05

		1820		94.03

		1819		94.01

		1818		93.99

		1817		93.98

		1816		93.96

		1815		93.95

		1814		93.94

		1813		93.93

		1812		93.92

		1811		93.91

		1810		93.9

		1809		93.89

		1808		93.88

		1807		93.87

		1806		93.86

		1805		93.85

		1804		93.84

		1803		93.83

		1802		93.81

		1801		93.79

		1800		93.77

		1799		93.74

		1798		93.71

		1797		93.68

		1796		93.64

		1795		93.6

		1794		93.56

		1793		93.51

		1792		93.47

		1791		93.42

		1790		93.38

		1789		93.35

		1788		93.32

		1787		93.29

		1786		93.28

		1785		93.27

		1784		93.28

		1783		93.29

		1782		93.31

		1781		93.34

		1780		93.38

		1779		93.41

		1778		93.46

		1777		93.5

		1776		93.54

		1775		93.59

		1774		93.63

		1773		93.67

		1772		93.7

		1771		93.74

		1770		93.77

		1769		93.8

		1768		93.83

		1767		93.86

		1766		93.89

		1765		93.91

		1764		93.94

		1763		93.96

		1762		93.98

		1761		94.01

		1760		94.02

		1759		94.04

		1758		94.06

		1757		94.07

		1756		94.08

		1755		94.09

		1754		94.1

		1753		94.1

		1752		94.09

		1751		94.09

		1750		94.08

		1749		94.06

		1748		94.04

		1747		94.01

		1746		93.98

		1745		93.94

		1744		93.89

		1743		93.83

		1742		93.77

		1741		93.69

		1740		93.6

		1739		93.5

		1738		93.4

		1737		93.27

		1736		93.13

		1735		92.98

		1734		92.81

		1733		92.61

		1732		92.39

		1731		92.13

		1730		91.85

		1729		91.52

		1728		91.15

		1727		90.71

		1726		90.2

		1725		89.61

		1724		88.93

		1723		88.15

		1722		87.27

		1721		86.29

		1720		85.2

		1719		84.01

		1718		82.71

		1717		81.32

		1716		79.85

		1715		78.31

		1714		76.69

		1713		75.01

		1712		73.27

		1711		71.49

		1710		69.66

		1709		67.8

		1708		65.93

		1707		64.07

		1706		62.24

		1705		60.48

		1704		58.82

		1703		57.29

		1702		55.92

		1701		54.72

		1700		53.7

		1699		52.89

		1698		52.3

		1697		51.9

		1696		51.68

		1695		51.61

		1694		51.67

		1693		51.85

		1692		52.15

		1691		52.54

		1690		53.03

		1689		53.62

		1688		54.3

		1687		55.1

		1686		56.02

		1685		57.08

		1684		58.29

		1683		59.65

		1682		61.14

		1681		62.75

		1680		64.45

		1679		66.22

		1678		68.04

		1677		69.87

		1676		71.68

		1675		73.44

		1674		75.12

		1673		76.69

		1672		78.15

		1671		79.49

		1670		80.72

		1669		81.83

		1668		82.82

		1667		83.7

		1666		84.47

		1665		85.16

		1664		85.78

		1663		86.33

		1662		86.82

		1661		87.27

		1660		87.67

		1659		88.02

		1658		88.35

		1657		88.64

		1656		88.91

		1655		89.16

		1654		89.39

		1653		89.6

		1652		89.79

		1651		89.97

		1650		90.14

		1649		90.29

		1648		90.44

		1647		90.59

		1646		90.72

		1645		90.85

		1644		90.98

		1643		91.1

		1642		91.22

		1641		91.33

		1640		91.45

		1639		91.55

		1638		91.66

		1637		91.76

		1636		91.86

		1635		91.96

		1634		92.05

		1633		92.14

		1632		92.23

		1631		92.31

		1630		92.39

		1629		92.47

		1628		92.55

		1627		92.63

		1626		92.7

		1625		92.77

		1624		92.84

		1623		92.91

		1622		92.98

		1621		93.04

		1620		93.11

		1619		93.17

		1618		93.24

		1617		93.3

		1616		93.36

		1615		93.42

		1614		93.48

		1613		93.53

		1612		93.59

		1611		93.64

		1610		93.68

		1609		93.73

		1608		93.77

		1607		93.81

		1606		93.85

		1605		93.89

		1604		93.92

		1603		93.95

		1602		93.98

		1601		94

		1600		94.02

		1599		94.05

		1598		94.07

		1597		94.09

		1596		94.1

		1595		94.12

		1594		94.14

		1593		94.16

		1592		94.18

		1591		94.2

		1590		94.21

		1589		94.23

		1588		94.25

		1587		94.27

		1586		94.28

		1585		94.3

		1584		94.31

		1583		94.32

		1582		94.33

		1581		94.34

		1580		94.35

		1579		94.36

		1578		94.37

		1577		94.37

		1576		94.38

		1575		94.38

		1574		94.38

		1573		94.38

		1572		94.38

		1571		94.38

		1570		94.39

		1569		94.39

		1568		94.39

		1567		94.39

		1566		94.4

		1565		94.4

		1564		94.41

		1563		94.42

		1562		94.43

		1561		94.44

		1560		94.45

		1559		94.46

		1558		94.47

		1557		94.47

		1556		94.48

		1555		94.48

		1554		94.49

		1553		94.49

		1552		94.5

		1551		94.5

		1550		94.5

		1549		94.5

		1548		94.5

		1547		94.5

		1546		94.5

		1545		94.51

		1544		94.51

		1543		94.51

		1542		94.52

		1541		94.52

		1540		94.53

		1539		94.54

		1538		94.55

		1537		94.56

		1536		94.57

		1535		94.57

		1534		94.58

		1533		94.58

		1532		94.59

		1531		94.59

		1530		94.59

		1529		94.59

		1528		94.58

		1527		94.58

		1526		94.57

		1525		94.56

		1524		94.56

		1523		94.55

		1522		94.54

		1521		94.53

		1520		94.52

		1519		94.51

		1518		94.5

		1517		94.5

		1516		94.49

		1515		94.48

		1514		94.47

		1513		94.47

		1512		94.46

		1511		94.46

		1510		94.46

		1509		94.45

		1508		94.45

		1507		94.45

		1506		94.45

		1505		94.44

		1504		94.44

		1503		94.43

		1502		94.43

		1501		94.42

		1500		94.41

		1499		94.4

		1498		94.38

		1497		94.37

		1496		94.35

		1495		94.33

		1494		94.31

		1493		94.29

		1492		94.27

		1491		94.24

		1490		94.2

		1489		94.16

		1488		94.1

		1487		94.03

		1486		93.93

		1485		93.79

		1484		93.59

		1483		93.3

		1482		92.87

		1481		92.28

		1480		91.54

		1479		90.66

		1478		89.67

		1477		88.59

		1476		87.45

		1475		86.27

		1474		85.1

		1473		83.99

		1472		83.03

		1471		82.27

		1470		81.75

		1469		81.42

		1468		81.25

		1467		81.22

		1466		81.29

		1465		81.48

		1464		81.77

		1463		82.15

		1462		82.58

		1461		83.02

		1460		83.44

		1459		83.85

		1458		84.26

		1457		84.69

		1456		85.11

		1455		85.52

		1454		85.89

		1453		86.21

		1452		86.46

		1451		86.65

		1450		86.78

		1449		86.83

		1448		86.83

		1447		86.76

		1446		86.64

		1445		86.45

		1444		86.22

		1443		85.93

		1442		85.59

		1441		85.19

		1440		84.75

		1439		84.27

		1438		83.76

		1437		83.22

		1436		82.67

		1435		82.14

		1434		81.65

		1433		81.22

		1432		80.87

		1431		80.63

		1430		80.5

		1429		80.5

		1428		80.63

		1427		80.87

		1426		81.21

		1425		81.62

		1424		82.06

		1423		82.5

		1422		82.89

		1421		83.21

		1420		83.42

		1419		83.52

		1418		83.5

		1417		83.36

		1416		83.14

		1415		82.84

		1414		82.53

		1413		82.23

		1412		82

		1411		81.89

		1410		81.9

		1409		82.07

		1408		82.4

		1407		82.86

		1406		83.46

		1405		84.15

		1404		84.92

		1403		85.71

		1402		86.51

		1401		87.28

		1400		88

		1399		88.65

		1398		89.23

		1397		89.73

		1396		90.15

		1395		90.52

		1394		90.82

		1393		91.07

		1392		91.28

		1391		91.45

		1390		91.58

		1389		91.68

		1388		91.76

		1387		91.81

		1386		91.83

		1385		91.83

		1384		91.81

		1383		91.76

		1382		91.69

		1381		91.6

		1380		91.51

		1379		91.4

		1378		91.3

		1377		91.2

		1376		91.11

		1375		91.02

		1374		90.95

		1373		90.88

		1372		90.83

		1371		90.79

		1370		90.75

		1369		90.69

		1368		90.62

		1367		90.53

		1366		90.42

		1365		90.28

		1364		90.11

		1363		89.93

		1362		89.72

		1361		89.5

		1360		89.27

		1359		89.04

		1358		88.82

		1357		88.62

		1356		88.44

		1355		88.29

		1354		88.16

		1353		88.08

		1352		88.04

		1351		88.04

		1350		88.09

		1349		88.2

		1348		88.35

		1347		88.55

		1346		88.79

		1345		89.04

		1344		89.3

		1343		89.55

		1342		89.76

		1341		89.93

		1340		90.02

		1339		90.04

		1338		89.97

		1337		89.82

		1336		89.59

		1335		89.3

		1334		88.98

		1333		88.65

		1332		88.33

		1331		88.05

		1330		87.83

		1329		87.69

		1328		87.63

		1327		87.64

		1326		87.71

		1325		87.81

		1324		87.91

		1323		87.99

		1322		88

		1321		87.91

		1320		87.69

		1319		87.31

		1318		86.78

		1317		86.1

		1316		85.27

		1315		84.33

		1314		83.31

		1313		82.24

		1312		81.18

		1311		80.15

		1310		79.22

		1309		78.4

		1308		77.73

		1307		77.22

		1306		76.86

		1305		76.65

		1304		76.54

		1303		76.53

		1302		76.57

		1301		76.65

		1300		76.72

		1299		76.75

		1298		76.72

		1297		76.6

		1296		76.38

		1295		76.07

		1294		75.7

		1293		75.3

		1292		74.9

		1291		74.52

		1290		74.2

		1289		73.97

		1288		73.88

		1287		73.96

		1286		74.23

		1285		74.72

		1284		75.4

		1283		76.25

		1282		77.23

		1281		78.31

		1280		79.44

		1279		80.59

		1278		81.71

		1277		82.76

		1276		83.69

		1275		84.48

		1274		85.09

		1273		85.51

		1272		85.74

		1271		85.79

		1270		85.65

		1269		85.38

		1268		84.98

		1267		84.51

		1266		84

		1265		83.5

		1264		83.06

		1263		82.75

		1262		82.59

		1261		82.62

		1260		82.85

		1259		83.25

		1258		83.8

		1257		84.46

		1256		85.21

		1255		85.99

		1254		86.77

		1253		87.49

		1252		88.13

		1251		88.64

		1250		89

		1249		89.2

		1248		89.2

		1247		89.01

		1246		88.64

		1245		88.09

		1244		87.4

		1243		86.61

		1242		85.74

		1241		84.85

		1240		84.01

		1239		83.27

		1238		82.7

		1237		82.36

		1236		82.26

		1235		82.41

		1234		82.78

		1233		83.34

		1232		84.03

		1231		84.82

		1230		85.65

		1229		86.46

		1228		87.2

		1227		87.82

		1226		88.29

		1225		88.59

		1224		88.71

		1223		88.65

		1222		88.43

		1221		88.06

		1220		87.57

		1219		86.99

		1218		86.35

		1217		85.68

		1216		85.04

		1215		84.48

		1214		84.04

		1213		83.77

		1212		83.68

		1211		83.77

		1210		84.04

		1209		84.46

		1208		85.02

		1207		85.69

		1206		86.42

		1205		87.15

		1204		87.85

		1203		88.44

		1202		88.9

		1201		89.18

		1200		89.27

		1199		89.17

		1198		88.89

		1197		88.47

		1196		87.93

		1195		87.33

		1194		86.71

		1193		86.13

		1192		85.64

		1191		85.32

		1190		85.2

		1189		85.29

		1188		85.59

		1187		86.06

		1186		86.66

		1185		87.35

		1184		88.09

		1183		88.84

		1182		89.58

		1181		90.25

		1180		90.84

		1179		91.34

		1178		91.75

		1177		92.07

		1176		92.34

		1175		92.55

		1174		92.73

		1173		92.88

		1172		93.01

		1171		93.13

		1170		93.23

		1169		93.32

		1168		93.4

		1167		93.47

		1166		93.54

		1165		93.6

		1164		93.65

		1163		93.7

		1162		93.75

		1161		93.79

		1160		93.83

		1159		93.87

		1158		93.9

		1157		93.93

		1156		93.96

		1155		93.99

		1154		94.02

		1153		94.04

		1152		94.06

		1151		94.08

		1150		94.1

		1149		94.12

		1148		94.13

		1147		94.15

		1146		94.16

		1145		94.17

		1144		94.19

		1143		94.2

		1142		94.2

		1141		94.21

		1140		94.21

		1139		94.21

		1138		94.19

		1137		94.17

		1136		94.13

		1135		94.08

		1134		94.01

		1133		93.92

		1132		93.82

		1131		93.7

		1130		93.57

		1129		93.43

		1128		93.3

		1127		93.18

		1126		93.08

		1125		93

		1124		92.95

		1123		92.93

		1122		92.94

		1121		92.99

		1120		93.05

		1119		93.13

		1118		93.22

		1117		93.31

		1116		93.4

		1115		93.48

		1114		93.54

		1113		93.59

		1112		93.63

		1111		93.65

		1110		93.66

		1109		93.66

		1108		93.66

		1107		93.64

		1106		93.61

		1105		93.55

		1104		93.46

		1103		93.32

		1102		93.12

		1101		92.86

		1100		92.55

		1099		92.2

		1098		91.82

		1097		91.42

		1096		91.02

		1095		90.66

		1094		90.35

		1093		90.12

		1092		89.99

		1091		89.97

		1090		90.05

		1089		90.2

		1088		90.42

		1087		90.67

		1086		90.94

		1085		91.21

		1084		91.47

		1083		91.69

		1082		91.87

		1081		92.01

		1080		92.1

		1079		92.16

		1078		92.2

		1077		92.21

		1076		92.21

		1075		92.2

		1074		92.18

		1073		92.15

		1072		92.12

		1071		92.09

		1070		92.05

		1069		92

		1068		91.95

		1067		91.91

		1066		91.86

		1065		91.82

		1064		91.78

		1063		91.75

		1062		91.71

		1061		91.67

		1060		91.64

		1059		91.6

		1058		91.57

		1057		91.55

		1056		91.53

		1055		91.51

		1054		91.51

		1053		91.5

		1052		91.51

		1051		91.53

		1050		91.55

		1049		91.57

		1048		91.59

		1047		91.61

		1046		91.62

		1045		91.63

		1044		91.63

		1043		91.62

		1042		91.61

		1041		91.59

		1040		91.58

		1039		91.57

		1038		91.58

		1037		91.59

		1036		91.62

		1035		91.65

		1034		91.7

		1033		91.77

		1032		91.85

		1031		91.93

		1030		92

		1029		92.07

		1028		92.12

		1027		92.17

		1026		92.2

		1025		92.23

		1024		92.25

		1023		92.25

		1022		92.24

		1021		92.23

		1020		92.22

		1019		92.2

		1018		92.19

		1017		92.17

		1016		92.15

		1015		92.13

		1014		92.1

		1013		92.08

		1012		92.05

		1011		92.01

		1010		91.97

		1009		91.92

		1008		91.87

		1007		91.81

		1006		91.76

		1005		91.7

		1004		91.65

		1003		91.6

		1002		91.56

		1001		91.53

		1000		91.51

		999		91.51

		998		91.52

		997		91.53

		996		91.55

		995		91.57

		994		91.58

		993		91.58

		992		91.57

		991		91.54

		990		91.51

		989		91.46

		988		91.4

		987		91.33

		986		91.26

		985		91.19

		984		91.12

		983		91.05

		982		90.97

		981		90.88

		980		90.77

		979		90.64

		978		90.48

		977		90.29

		976		90.07

		975		89.82

		974		89.53

		973		89.2

		972		88.85

		971		88.46

		970		88.06

		969		87.64

		968		87.2

		967		86.76

		966		86.31

		965		85.85

		964		85.39

		963		84.93

		962		84.47

		961		84.01

		960		83.55

		959		83.09

		958		82.62

		957		82.16

		956		81.68

		955		81.19

		954		80.7

		953		80.19

		952		79.66

		951		79.11

		950		78.55

		949		77.96

		948		77.36

		947		76.76

		946		76.16

		945		75.58

		944		75.04

		943		74.53

		942		74.09

		941		73.73

		940		73.45

		939		73.27

		938		73.2

		937		73.24

		936		73.39

		935		73.65

		934		74.01

		933		74.46

		932		74.99

		931		75.58

		930		76.23

		929		76.91

		928		77.62

		927		78.34

		926		79.05

		925		79.76

		924		80.43

		923		81.07

		922		81.66

		921		82.19

		920		82.67

		919		83.08

		918		83.42

		917		83.69

		916		83.89

		915		84.04

		914		84.14

		913		84.21

		912		84.26

		911		84.31

		910		84.37

		909		84.45

		908		84.57

		907		84.71

		906		84.9

		905		85.11

		904		85.33

		903		85.56

		902		85.78

		901		85.96

		900		86.12

		899		86.22

		898		86.29

		897		86.3

		896		86.27

		895		86.21

		894		86.13

		893		86.06

		892		85.99

		891		85.95

		890		85.95

		889		85.99

		888		86.07

		887		86.21

		886		86.39

		885		86.62

		884		86.87

		883		87.14

		882		87.42

		881		87.71

		880		87.98

		879		88.25

		878		88.51

		877		88.74

		876		88.96

		875		89.16

		874		89.35

		873		89.52

		872		89.68

		871		89.84

		870		89.98

		869		90.12

		868		90.26

		867		90.38

		866		90.51

		865		90.63

		864		90.75

		863		90.87

		862		90.99

		861		91.11

		860		91.23

		859		91.36

		858		91.49

		857		91.63

		856		91.77

		855		91.9

		854		92.03

		853		92.16

		852		92.28

		851		92.4

		850		92.51

		849		92.61

		848		92.71

		847		92.8

		846		92.88

		845		92.96

		844		93.03

		843		93.09

		842		93.16

		841		93.22

		840		93.28

		839		93.33

		838		93.38

		837		93.43

		836		93.48

		835		93.52

		834		93.56

		833		93.6

		832		93.63

		831		93.66

		830		93.68

		829		93.69

		828		93.68

		827		93.66

		826		93.61

		825		93.53

		824		93.41

		823		93.26

		822		93.07

		821		92.87

		820		92.67

		819		92.47

		818		92.29

		817		92.14

		816		92.04

		815		92.01

		814		92.05

		813		92.17

		812		92.36

		811		92.59

		810		92.85

		809		93.12

		808		93.39

		807		93.65

		806		93.89

		805		94.1

		804		94.27

		803		94.41

		802		94.51

		801		94.59

		800		94.65

		799		94.69

		798		94.73

		797		94.76

		796		94.79

		795		94.8

		794		94.81

		793		94.8

		792		94.78

		791		94.74

		790		94.68

		789		94.6

		788		94.51

		787		94.42

		786		94.32

		785		94.23

		784		94.15

		783		94.08

		782		94.05

		781		94.04

		780		94.07

		779		94.14

		778		94.22

		777		94.32

		776		94.43

		775		94.54

		774		94.65

		773		94.74

		772		94.83

		771		94.89

		770		94.94

		769		94.96

		768		94.97

		767		94.95

		766		94.92

		765		94.85

		764		94.75

		763		94.6

		762		94.41

		761		94.17

		760		93.9

		759		93.61

		758		93.31

		757		93.03

		756		92.78

		755		92.57

		754		92.43

		753		92.38

		752		92.42

		751		92.55

		750		92.75

		749		92.99

		748		93.24

		747		93.49

		746		93.72

		745		93.91

		744		94.04

		743		94.1

		742		94.09

		741		93.97

		740		93.76

		739		93.42

		738		92.96

		737		92.35

		736		91.6

		735		90.72

		734		89.71

		733		88.61

		732		87.42

		731		86.18

		730		84.9

		729		83.65

		728		82.48

		727		81.49

		726		80.7

		725		80.16

		724		79.86

		723		79.79

		722		79.96

		721		80.36

		720		81.01

		719		81.88

		718		82.92

		717		84.06

		716		85.23

		715		86.38

		714		87.48

		713		88.51

		712		89.44

		711		90.26

		710		90.95

		709		91.5

		708		91.9

		707		92.18

		706		92.36

		705		92.45

		704		92.47

		703		92.42

		702		92.31

		701		92.12

		700		91.86

		699		91.53

		698		91.13

		697		90.65

		696		90.11

		695		89.52

		694		88.91

		693		88.29

		692		87.68

		691		87.12

		690		86.63

		689		86.22

		688		85.92

		687		85.73

		686		85.66

		685		85.69

		684		85.81

		683		86.02

		682		86.27

		681		86.57

		680		86.89

		679		87.2

		678		87.51

		677		87.8

		676		88.07

		675		88.31

		674		88.54

		673		88.76

		672		88.96

		671		89.16

		670		89.37

		669		89.58

		668		89.8

		667		90.03

		666		90.26

		665		90.51

		664		90.76

		663		91.02

		662		91.28

		661		91.54

		660		91.79

		659		92.04

		658		92.28

		657		92.51

		656		92.72

		655		92.92

		654		93.1

		653		93.26

		652		93.41

		651		93.54

		650		93.65

		649		93.75

		648		93.83

		647		93.89

		646		93.95

		645		93.99

		644		94.02

		643		94.04

		642		94.06

		641		94.08

		640		94.1

		639		94.11

		638		94.13

		637		94.16

		636		94.19

		635		94.22

		634		94.27

		633		94.31

		632		94.37

		631		94.42

		630		94.48

		629		94.54

		628		94.59

		627		94.65

		626		94.7

		625		94.75

		624		94.8

		623		94.83

		622		94.87

		621		94.9

		620		94.92

		619		94.95

		618		94.96

		617		94.98

		616		94.99

		615		95

		614		95.01

		613		95.02

		612		95.03

		611		95.04

		610		95.05

		609		95.06

		608		95.07

		607		95.08

		606		95.09

		605		95.1

		604		95.11

		603		95.13

		602		95.14

		601		95.15

		600		95.16

		599		95.16

		598		95.17

		597		95.17

		596		95.17

		595		95.18

		594		95.18

		593		95.18

		592		95.17

		591		95.17

		590		95.17

		589		95.17

		588		95.16

		587		95.16

		586		95.14

		585		95.13

		584		95.1

		583		95.07

		582		95.04

		581		94.99

		580		94.94

		579		94.87

		578		94.79

		577		94.7

		576		94.59

		575		94.47

		574		94.34

		573		94.19

		572		94.02

		571		93.84

		570		93.64

		569		93.42

		568		93.18

		567		92.92

		566		92.65

		565		92.35

		564		92.02

		563		91.68

		562		91.31

		561		90.91

		560		90.5

		559		90.06

		558		89.6

		557		89.13

		556		88.66

		555		88.2

		554		87.75

		553		87.34

		552		86.99

		551		86.69

		550		86.48

		549		86.36

		548		86.34

		547		86.43

		546		86.62

		545		86.92

		544		87.31

		543		87.78

		542		88.31

		541		88.89

		540		89.48

		539		90.09

		538		90.68

		537		91.25

		536		91.78

		535		92.26

		534		92.69

		533		93.07

		532		93.39

		531		93.68

		530		93.91

		529		94.11

		528		94.27

		527		94.41

		526		94.52

		525		94.61

		524		94.7

		523		94.77

		522		94.83

		521		94.87

		520		94.92

		519		94.95

		518		94.98

		517		95

		516		95

		515		94.99

		514		94.95

		513		94.89

		512		94.78

		511		94.63

		510		94.42

		509		94.14

		508		93.81

		507		93.42

		506		92.99

		505		92.54

		504		92.09

		503		91.66

		502		91.28

		501		90.97

		500		90.77

		499		90.68

		498		90.7

		497		90.83

		496		91.05

		495		91.34

		494		91.68

		493		92.05

		492		92.42

		491		92.77

		490		93.09

		489		93.37

		488		93.59

		487		93.78

		486		93.92

		485		94.04

		484		94.14

		483		94.22

		482		94.3

		481		94.36

		480		94.43

		479		94.5

		478		94.57

		477		94.64

		476		94.71

		475		94.78

		474		94.84

		473		94.89

		472		94.94

		471		94.99

		470		95.03

		469		95.06

		468		95.09

		467		95.11

		466		95.12

		465		95.13

		464		95.15

		463		95.16

		462		95.17

		461		95.17

		460		95.17

		459		95.16

		458		95.16

		457		95.15

		456		95.13

		455		95.1

		454		95.05

		453		94.99

		452		94.9

		451		94.8

		450		94.66

		449		94.48

		448		94.25

		447		93.96

		446		93.6

		445		93.18

		444		92.71

		443		92.19

		442		91.66

		441		91.13

		440		90.62

		439		90.18

		438		89.83

		437		89.6

		436		89.5

		435		89.55

		434		89.75

		433		90.07

		432		90.5

		431		91

		430		91.54

		429		92.09

		428		92.63

		427		93.12

		426		93.56

		425		93.91

		424		94.19

		423		94.38

		422		94.49

		421		94.55

		420		94.56

		419		94.54

		418		94.5

		417		94.46

		416		94.42

		415		94.39

		414		94.38

		413		94.39

		412		94.42

		411		94.48

		410		94.55

		409		94.63

		408		94.72

		407		94.82

		406		94.92

		405		95.01

		404		95.1

		403		95.18

		402		95.26

		401		95.34

		400		95.43
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		cm-1		%T

		4000		94.76

		3999		94.76

		3998		94.76

		3997		94.76

		3996		94.76

		3995		94.76

		3994		94.76

		3993		94.76

		3992		94.76

		3991		94.76

		3990		94.76

		3989		94.76

		3988		94.76

		3987		94.75

		3986		94.75

		3985		94.75

		3984		94.75

		3983		94.75

		3982		94.75

		3981		94.75

		3980		94.75

		3979		94.75

		3978		94.75

		3977		94.75

		3976		94.75

		3975		94.75

		3974		94.75

		3973		94.75

		3972		94.75

		3971		94.75

		3970		94.75

		3969		94.75

		3968		94.75

		3967		94.75

		3966		94.76

		3965		94.76

		3964		94.76

		3963		94.76

		3962		94.76

		3961		94.76

		3960		94.76

		3959		94.76

		3958		94.76

		3957		94.76

		3956		94.76

		3955		94.76

		3954		94.76

		3953		94.76

		3952		94.76

		3951		94.76

		3950		94.75

		3949		94.75

		3948		94.75

		3947		94.75

		3946		94.75

		3945		94.75

		3944		94.75

		3943		94.75

		3942		94.75

		3941		94.75

		3940		94.75

		3939		94.75

		3938		94.75

		3937		94.75

		3936		94.75

		3935		94.75

		3934		94.75

		3933		94.76

		3932		94.76

		3931		94.76

		3930		94.76

		3929		94.76

		3928		94.76

		3927		94.76

		3926		94.75

		3925		94.75

		3924		94.75

		3923		94.74

		3922		94.74

		3921		94.73

		3920		94.73

		3919		94.73

		3918		94.72

		3917		94.72

		3916		94.72

		3915		94.72

		3914		94.72

		3913		94.72

		3912		94.72

		3911		94.72

		3910		94.72

		3909		94.72

		3908		94.71

		3907		94.71

		3906		94.71

		3905		94.71

		3904		94.7

		3903		94.7

		3902		94.7

		3901		94.7

		3900		94.7

		3899		94.7

		3898		94.7

		3897		94.7

		3896		94.7

		3895		94.7

		3894		94.7

		3893		94.7

		3892		94.7

		3891		94.7

		3890		94.7

		3889		94.7

		3888		94.7

		3887		94.7

		3886		94.7

		3885		94.7

		3884		94.7

		3883		94.7

		3882		94.7

		3881		94.7

		3880		94.7

		3879		94.7

		3878		94.7

		3877		94.7

		3876		94.7

		3875		94.7

		3874		94.7

		3873		94.7

		3872		94.69

		3871		94.69

		3870		94.69

		3869		94.69

		3868		94.69

		3867		94.69

		3866		94.69

		3865		94.69

		3864		94.69

		3863		94.69

		3862		94.69

		3861		94.69

		3860		94.69

		3859		94.69

		3858		94.69

		3857		94.7

		3856		94.7

		3855		94.7

		3854		94.7

		3853		94.7

		3852		94.7

		3851		94.7

		3850		94.7

		3849		94.7

		3848		94.7

		3847		94.7

		3846		94.7

		3845		94.7

		3844		94.7

		3843		94.69

		3842		94.69

		3841		94.69

		3840		94.69

		3839		94.69

		3838		94.69

		3837		94.69

		3836		94.69

		3835		94.69

		3834		94.69

		3833		94.69

		3832		94.7

		3831		94.7

		3830		94.7

		3829		94.7

		3828		94.7

		3827		94.71

		3826		94.71

		3825		94.71

		3824		94.71

		3823		94.71

		3822		94.71

		3821		94.71

		3820		94.71

		3819		94.71

		3818		94.71

		3817		94.71

		3816		94.71

		3815		94.72

		3814		94.72

		3813		94.71

		3812		94.71

		3811		94.71

		3810		94.71

		3809		94.71

		3808		94.7

		3807		94.7

		3806		94.7

		3805		94.7

		3804		94.7

		3803		94.7

		3802		94.7

		3801		94.7

		3800		94.71

		3799		94.71

		3798		94.71

		3797		94.71

		3796		94.72

		3795		94.72

		3794		94.72

		3793		94.73

		3792		94.73

		3791		94.73

		3790		94.74

		3789		94.74

		3788		94.74

		3787		94.75

		3786		94.75

		3785		94.75

		3784		94.75

		3783		94.76

		3782		94.76

		3781		94.76

		3780		94.76

		3779		94.76

		3778		94.76

		3777		94.76

		3776		94.76

		3775		94.76

		3774		94.76

		3773		94.76

		3772		94.76

		3771		94.76

		3770		94.75

		3769		94.75

		3768		94.75

		3767		94.75

		3766		94.74

		3765		94.74

		3764		94.74

		3763		94.74

		3762		94.74

		3761		94.73

		3760		94.73

		3759		94.73

		3758		94.72

		3757		94.71

		3756		94.71

		3755		94.7

		3754		94.69

		3753		94.68

		3752		94.68

		3751		94.67

		3750		94.67

		3749		94.67

		3748		94.67

		3747		94.67

		3746		94.67

		3745		94.68

		3744		94.68

		3743		94.68

		3742		94.69

		3741		94.69

		3740		94.7

		3739		94.7

		3738		94.7

		3737		94.71

		3736		94.71

		3735		94.71

		3734		94.71

		3733		94.71

		3732		94.72

		3731		94.72

		3730		94.72

		3729		94.72

		3728		94.72

		3727		94.72

		3726		94.72

		3725		94.71

		3724		94.71

		3723		94.71

		3722		94.7

		3721		94.7

		3720		94.69

		3719		94.68

		3718		94.67

		3717		94.66

		3716		94.64

		3715		94.63

		3714		94.62

		3713		94.61

		3712		94.6

		3711		94.59

		3710		94.58

		3709		94.57

		3708		94.56

		3707		94.55

		3706		94.54

		3705		94.53

		3704		94.52

		3703		94.51

		3702		94.49

		3701		94.48

		3700		94.46

		3699		94.45

		3698		94.43

		3697		94.41

		3696		94.4

		3695		94.38

		3694		94.37

		3693		94.35

		3692		94.34

		3691		94.33

		3690		94.31

		3689		94.3

		3688		94.29

		3687		94.28

		3686		94.27

		3685		94.26

		3684		94.25

		3683		94.23

		3682		94.22

		3681		94.21

		3680		94.19

		3679		94.18

		3678		94.17

		3677		94.16

		3676		94.15

		3675		94.14

		3674		94.14

		3673		94.13

		3672		94.13

		3671		94.13

		3670		94.13

		3669		94.13

		3668		94.14

		3667		94.14

		3666		94.14

		3665		94.15

		3664		94.15

		3663		94.16

		3662		94.16

		3661		94.17

		3660		94.18

		3659		94.19

		3658		94.2

		3657		94.21

		3656		94.23

		3655		94.24

		3654		94.25

		3653		94.27

		3652		94.29

		3651		94.3

		3650		94.32

		3649		94.34

		3648		94.36

		3647		94.37

		3646		94.39

		3645		94.41

		3644		94.43

		3643		94.45

		3642		94.47

		3641		94.49

		3640		94.51

		3639		94.52

		3638		94.54

		3637		94.55

		3636		94.56

		3635		94.57

		3634		94.58

		3633		94.59

		3632		94.59

		3631		94.6

		3630		94.61

		3629		94.62

		3628		94.63

		3627		94.64

		3626		94.65

		3625		94.66

		3624		94.67

		3623		94.67

		3622		94.68

		3621		94.68

		3620		94.69

		3619		94.69

		3618		94.69

		3617		94.68

		3616		94.68

		3615		94.67

		3614		94.67

		3613		94.66

		3612		94.66

		3611		94.65

		3610		94.65

		3609		94.65

		3608		94.65

		3607		94.65

		3606		94.65

		3605		94.66

		3604		94.66

		3603		94.67

		3602		94.68

		3601		94.69

		3600		94.69

		3599		94.7

		3598		94.71

		3597		94.71

		3596		94.72

		3595		94.72

		3594		94.73

		3593		94.73

		3592		94.73

		3591		94.73

		3590		94.74

		3589		94.74

		3588		94.74

		3587		94.75

		3586		94.75

		3585		94.75

		3584		94.76

		3583		94.76

		3582		94.76

		3581		94.76

		3580		94.76

		3579		94.76

		3578		94.76

		3577		94.76

		3576		94.76

		3575		94.76

		3574		94.76

		3573		94.76

		3572		94.76

		3571		94.76

		3570		94.76

		3569		94.76

		3568		94.76

		3567		94.75

		3566		94.75

		3565		94.75

		3564		94.75

		3563		94.75

		3562		94.75

		3561		94.75

		3560		94.74

		3559		94.74

		3558		94.74

		3557		94.74

		3556		94.74

		3555		94.73

		3554		94.73

		3553		94.73

		3552		94.73

		3551		94.72

		3550		94.72

		3549		94.72

		3548		94.72

		3547		94.72

		3546		94.71

		3545		94.71

		3544		94.71

		3543		94.71

		3542		94.71

		3541		94.71

		3540		94.7

		3539		94.7

		3538		94.7

		3537		94.7

		3536		94.7

		3535		94.69

		3534		94.69

		3533		94.69

		3532		94.69

		3531		94.69

		3530		94.69

		3529		94.69

		3528		94.69

		3527		94.69

		3526		94.7

		3525		94.7

		3524		94.7

		3523		94.7

		3522		94.7

		3521		94.69

		3520		94.69

		3519		94.69

		3518		94.69

		3517		94.69

		3516		94.68

		3515		94.68

		3514		94.68

		3513		94.67

		3512		94.67

		3511		94.67

		3510		94.66

		3509		94.66

		3508		94.66

		3507		94.65

		3506		94.65

		3505		94.65

		3504		94.65

		3503		94.65

		3502		94.65

		3501		94.65

		3500		94.65

		3499		94.65

		3498		94.65

		3497		94.65

		3496		94.65

		3495		94.65

		3494		94.64

		3493		94.64

		3492		94.64

		3491		94.64

		3490		94.64

		3489		94.64

		3488		94.63

		3487		94.63

		3486		94.63

		3485		94.63

		3484		94.63

		3483		94.63

		3482		94.62

		3481		94.62

		3480		94.62

		3479		94.62

		3478		94.61

		3477		94.61

		3476		94.61

		3475		94.61

		3474		94.61

		3473		94.61

		3472		94.61

		3471		94.6

		3470		94.6

		3469		94.6

		3468		94.6

		3467		94.6

		3466		94.6

		3465		94.6

		3464		94.59

		3463		94.59

		3462		94.59

		3461		94.59

		3460		94.58

		3459		94.58

		3458		94.58

		3457		94.57

		3456		94.57

		3455		94.57

		3454		94.57

		3453		94.57

		3452		94.56

		3451		94.56

		3450		94.56

		3449		94.56

		3448		94.56

		3447		94.55

		3446		94.55

		3445		94.55

		3444		94.55

		3443		94.55

		3442		94.55

		3441		94.55

		3440		94.55

		3439		94.55

		3438		94.55

		3437		94.55

		3436		94.54

		3435		94.54

		3434		94.53

		3433		94.53

		3432		94.52

		3431		94.51

		3430		94.5

		3429		94.49

		3428		94.49

		3427		94.48

		3426		94.47

		3425		94.46

		3424		94.45

		3423		94.44

		3422		94.44

		3421		94.43

		3420		94.43

		3419		94.43

		3418		94.42

		3417		94.42

		3416		94.42

		3415		94.42

		3414		94.41

		3413		94.41

		3412		94.41

		3411		94.41

		3410		94.41

		3409		94.41

		3408		94.41

		3407		94.41

		3406		94.41

		3405		94.41

		3404		94.42

		3403		94.42

		3402		94.42

		3401		94.43

		3400		94.43

		3399		94.43

		3398		94.43

		3397		94.42

		3396		94.42

		3395		94.41

		3394		94.4

		3393		94.4

		3392		94.38

		3391		94.37

		3390		94.36

		3389		94.35

		3388		94.34

		3387		94.33

		3386		94.32

		3385		94.31

		3384		94.31

		3383		94.3

		3382		94.3

		3381		94.3

		3380		94.31

		3379		94.31

		3378		94.32

		3377		94.33

		3376		94.33

		3375		94.34

		3374		94.35

		3373		94.35

		3372		94.36

		3371		94.36

		3370		94.37

		3369		94.37

		3368		94.37

		3367		94.36

		3366		94.35

		3365		94.35

		3364		94.34

		3363		94.33

		3362		94.32

		3361		94.31

		3360		94.31

		3359		94.3

		3358		94.3

		3357		94.29

		3356		94.29

		3355		94.29

		3354		94.29

		3353		94.29

		3352		94.29

		3351		94.29

		3350		94.29

		3349		94.29

		3348		94.28

		3347		94.28

		3346		94.28

		3345		94.28

		3344		94.27

		3343		94.27

		3342		94.27

		3341		94.26

		3340		94.26

		3339		94.26

		3338		94.25

		3337		94.25

		3336		94.24

		3335		94.24

		3334		94.23

		3333		94.23

		3332		94.22

		3331		94.22

		3330		94.21

		3329		94.21

		3328		94.21

		3327		94.21

		3326		94.2

		3325		94.2

		3324		94.2

		3323		94.2

		3322		94.2

		3321		94.2

		3320		94.2

		3319		94.2

		3318		94.2

		3317		94.2

		3316		94.2

		3315		94.2

		3314		94.2

		3313		94.2

		3312		94.21

		3311		94.21

		3310		94.21

		3309		94.21

		3308		94.21

		3307		94.21

		3306		94.21

		3305		94.2

		3304		94.2

		3303		94.2

		3302		94.19

		3301		94.19

		3300		94.18

		3299		94.17

		3298		94.17

		3297		94.16

		3296		94.16

		3295		94.15

		3294		94.14

		3293		94.14

		3292		94.13

		3291		94.12

		3290		94.11

		3289		94.1

		3288		94.1

		3287		94.09

		3286		94.08

		3285		94.07

		3284		94.06

		3283		94.06

		3282		94.05

		3281		94.05

		3280		94.04

		3279		94.04

		3278		94.03

		3277		94.02

		3276		94.02

		3275		94.01

		3274		94

		3273		93.99

		3272		93.98

		3271		93.97

		3270		93.96

		3269		93.95

		3268		93.94

		3267		93.93

		3266		93.92

		3265		93.91

		3264		93.9

		3263		93.89

		3262		93.88

		3261		93.87

		3260		93.86

		3259		93.86

		3258		93.85

		3257		93.84

		3256		93.83

		3255		93.81

		3254		93.8

		3253		93.79

		3252		93.78

		3251		93.77

		3250		93.76

		3249		93.75

		3248		93.73

		3247		93.72

		3246		93.71

		3245		93.7

		3244		93.69

		3243		93.68

		3242		93.66

		3241		93.65

		3240		93.64

		3239		93.63

		3238		93.61

		3237		93.6

		3236		93.59

		3235		93.57

		3234		93.56

		3233		93.54

		3232		93.53

		3231		93.51

		3230		93.5

		3229		93.48

		3228		93.46

		3227		93.45

		3226		93.43

		3225		93.42

		3224		93.4

		3223		93.39

		3222		93.38

		3221		93.36

		3220		93.35

		3219		93.33

		3218		93.32

		3217		93.31

		3216		93.29

		3215		93.28

		3214		93.26

		3213		93.25

		3212		93.23

		3211		93.22

		3210		93.2

		3209		93.19

		3208		93.17

		3207		93.16

		3206		93.14

		3205		93.13

		3204		93.11

		3203		93.1

		3202		93.08

		3201		93.07

		3200		93.05

		3199		93.04

		3198		93.03

		3197		93.01

		3196		93

		3195		92.99

		3194		92.97

		3193		92.96

		3192		92.95

		3191		92.94

		3190		92.92

		3189		92.91

		3188		92.89

		3187		92.88

		3186		92.87

		3185		92.85

		3184		92.84

		3183		92.82

		3182		92.81

		3181		92.79

		3180		92.78

		3179		92.77

		3178		92.75

		3177		92.74

		3176		92.73

		3175		92.72

		3174		92.7

		3173		92.69

		3172		92.68

		3171		92.66

		3170		92.65

		3169		92.63

		3168		92.62

		3167		92.6

		3166		92.59

		3165		92.57

		3164		92.56

		3163		92.54

		3162		92.52

		3161		92.51

		3160		92.49

		3159		92.47

		3158		92.45

		3157		92.43

		3156		92.41

		3155		92.39

		3154		92.37

		3153		92.35

		3152		92.33

		3151		92.31

		3150		92.29

		3149		92.26

		3148		92.24

		3147		92.22

		3146		92.19

		3145		92.17

		3144		92.15

		3143		92.12

		3142		92.1

		3141		92.07

		3140		92.04

		3139		92.02

		3138		91.99

		3137		91.96

		3136		91.94

		3135		91.91

		3134		91.88

		3133		91.85

		3132		91.83

		3131		91.8

		3130		91.77

		3129		91.74

		3128		91.71

		3127		91.68

		3126		91.66

		3125		91.63

		3124		91.6

		3123		91.57

		3122		91.55

		3121		91.52

		3120		91.49

		3119		91.46

		3118		91.43

		3117		91.41

		3116		91.38

		3115		91.35

		3114		91.32

		3113		91.29

		3112		91.26

		3111		91.22

		3110		91.19

		3109		91.16

		3108		91.13

		3107		91.1

		3106		91.07

		3105		91.04

		3104		91.01

		3103		90.98

		3102		90.95

		3101		90.92

		3100		90.9

		3099		90.87

		3098		90.85

		3097		90.82

		3096		90.8

		3095		90.78

		3094		90.75

		3093		90.73

		3092		90.71

		3091		90.69

		3090		90.67

		3089		90.65

		3088		90.63

		3087		90.61

		3086		90.59

		3085		90.57

		3084		90.55

		3083		90.53

		3082		90.51

		3081		90.49

		3080		90.47

		3079		90.45

		3078		90.43

		3077		90.41

		3076		90.39

		3075		90.37

		3074		90.35

		3073		90.33

		3072		90.3

		3071		90.28

		3070		90.26

		3069		90.24

		3068		90.21

		3067		90.19

		3066		90.17

		3065		90.14

		3064		90.12

		3063		90.09

		3062		90.07

		3061		90.04

		3060		90.01

		3059		89.98

		3058		89.95

		3057		89.92

		3056		89.89

		3055		89.86

		3054		89.82

		3053		89.78

		3052		89.75

		3051		89.71

		3050		89.67

		3049		89.63

		3048		89.58

		3047		89.54

		3046		89.49

		3045		89.45

		3044		89.4

		3043		89.35

		3042		89.3

		3041		89.24

		3040		89.19

		3039		89.13

		3038		89.07

		3037		89.01

		3036		88.95

		3035		88.89

		3034		88.83

		3033		88.77

		3032		88.71

		3031		88.65

		3030		88.59

		3029		88.52

		3028		88.46

		3027		88.4

		3026		88.34

		3025		88.28

		3024		88.22

		3023		88.16

		3022		88.11

		3021		88.05

		3020		87.99

		3019		87.93

		3018		87.87

		3017		87.82

		3016		87.76

		3015		87.71

		3014		87.65

		3013		87.6

		3012		87.55

		3011		87.49

		3010		87.44

		3009		87.39

		3008		87.35

		3007		87.3

		3006		87.26

		3005		87.22

		3004		87.18

		3003		87.14

		3002		87.11

		3001		87.07

		3000		87.04

		2999		87

		2998		86.96

		2997		86.91

		2996		86.87

		2995		86.82

		2994		86.78

		2993		86.72

		2992		86.67

		2991		86.62

		2990		86.56

		2989		86.51

		2988		86.46

		2987		86.42

		2986		86.37

		2985		86.33

		2984		86.28

		2983		86.23

		2982		86.18

		2981		86.11

		2980		86.04

		2979		85.96

		2978		85.85

		2977		85.71

		2976		85.54

		2975		85.32

		2974		85.04

		2973		84.71

		2972		84.31

		2971		83.86

		2970		83.36

		2969		82.82

		2968		82.25

		2967		81.66

		2966		81.07

		2965		80.48

		2964		79.91

		2963		79.38

		2962		78.89

		2961		78.44

		2960		78.05

		2959		77.72

		2958		77.46

		2957		77.26

		2956		77.13

		2955		77.08

		2954		77.11

		2953		77.22

		2952		77.38

		2951		77.59

		2950		77.82

		2949		78.04

		2948		78.24

		2947		78.39

		2946		78.48

		2945		78.49

		2944		78.41

		2943		78.25

		2942		78.01

		2941		77.7

		2940		77.34

		2939		76.94

		2938		76.51

		2937		76.06

		2936		75.61

		2935		75.15

		2934		74.68

		2933		74.18

		2932		73.64

		2931		73.04

		2930		72.35

		2929		71.55

		2928		70.63

		2927		69.55

		2926		68.32

		2925		66.93

		2924		65.4

		2923		63.75

		2922		62.03

		2921		60.3

		2920		58.61

		2919		57.05

		2918		55.69

		2917		54.58

		2916		53.78

		2915		53.33

		2914		53.25

		2913		53.52

		2912		54.14

		2911		55.04

		2910		56.17

		2909		57.47

		2908		58.87

		2907		60.32

		2906		61.75

		2905		63.12

		2904		64.41

		2903		65.59

		2902		66.66

		2901		67.62

		2900		68.48

		2899		69.26

		2898		69.96

		2897		70.6

		2896		71.19

		2895		71.74

		2894		72.27

		2893		72.78

		2892		73.28

		2891		73.77

		2890		74.25

		2889		74.73

		2888		75.2

		2887		75.66

		2886		76.11

		2885		76.53

		2884		76.92

		2883		77.27

		2882		77.56

		2881		77.79

		2880		77.96

		2879		78.07

		2878		78.12

		2877		78.12

		2876		78.08

		2875		78.02

		2874		77.95

		2873		77.89

		2872		77.86

		2871		77.85

		2870		77.87

		2869		77.91

		2868		77.96

		2867		77.99

		2866		77.99

		2865		77.93

		2864		77.78

		2863		77.52

		2862		77.12

		2861		76.54

		2860		75.76

		2859		74.77

		2858		73.58

		2857		72.19

		2856		70.65

		2855		69.01

		2854		67.33

		2853		65.7

		2852		64.19

		2851		62.89

		2850		61.89

		2849		61.26

		2848		61.06

		2847		61.28

		2846		61.92

		2845		62.93

		2844		64.25

		2843		65.8

		2842		67.49

		2841		69.26

		2840		71.01

		2839		72.69

		2838		74.25

		2837		75.65

		2836		76.89

		2835		77.96

		2834		78.89

		2833		79.68

		2832		80.36

		2831		80.95

		2830		81.46

		2829		81.91

		2828		82.3

		2827		82.66

		2826		82.98

		2825		83.26

		2824		83.52

		2823		83.76

		2822		83.98

		2821		84.19

		2820		84.38

		2819		84.55

		2818		84.71

		2817		84.87

		2816		85.01

		2815		85.14

		2814		85.27

		2813		85.38

		2812		85.49

		2811		85.6

		2810		85.7

		2809		85.8

		2808		85.89

		2807		85.98

		2806		86.07

		2805		86.15

		2804		86.24

		2803		86.32

		2802		86.39

		2801		86.47

		2800		86.54

		2799		86.61

		2798		86.68

		2797		86.74

		2796		86.81

		2795		86.86

		2794		86.92

		2793		86.97

		2792		87.02

		2791		87.07

		2790		87.11

		2789		87.15

		2788		87.19

		2787		87.23

		2786		87.26

		2785		87.3

		2784		87.33

		2783		87.36

		2782		87.39

		2781		87.42

		2780		87.45

		2779		87.47

		2778		87.5

		2777		87.52

		2776		87.55

		2775		87.57

		2774		87.59

		2773		87.61

		2772		87.63

		2771		87.65

		2770		87.68

		2769		87.7

		2768		87.72

		2767		87.74

		2766		87.77

		2765		87.79

		2764		87.81

		2763		87.84

		2762		87.86

		2761		87.88

		2760		87.91

		2759		87.93

		2758		87.95

		2757		87.97

		2756		88

		2755		88.02

		2754		88.04

		2753		88.06

		2752		88.09

		2751		88.11

		2750		88.13

		2749		88.16

		2748		88.18

		2747		88.21

		2746		88.23

		2745		88.26

		2744		88.28

		2743		88.3

		2742		88.33

		2741		88.35

		2740		88.37

		2739		88.39

		2738		88.41

		2737		88.42

		2736		88.44

		2735		88.45

		2734		88.46

		2733		88.48

		2732		88.49

		2731		88.5

		2730		88.51

		2729		88.52

		2728		88.54

		2727		88.55

		2726		88.56

		2725		88.57

		2724		88.58

		2723		88.59

		2722		88.59

		2721		88.59

		2720		88.59

		2719		88.58

		2718		88.57

		2717		88.55

		2716		88.53

		2715		88.5

		2714		88.48

		2713		88.45

		2712		88.42

		2711		88.38

		2710		88.35

		2709		88.32

		2708		88.29

		2707		88.26

		2706		88.23

		2705		88.21

		2704		88.19

		2703		88.17

		2702		88.15

		2701		88.13

		2700		88.11

		2699		88.09

		2698		88.08

		2697		88.06

		2696		88.04

		2695		88.02

		2694		88

		2693		87.98

		2692		87.95

		2691		87.93

		2690		87.91

		2689		87.88

		2688		87.86

		2687		87.84

		2686		87.82

		2685		87.8

		2684		87.78

		2683		87.77

		2682		87.76

		2681		87.75

		2680		87.74

		2679		87.73

		2678		87.73

		2677		87.73

		2676		87.73

		2675		87.73

		2674		87.73

		2673		87.73

		2672		87.74

		2671		87.74

		2670		87.75

		2669		87.75

		2668		87.75

		2667		87.75

		2666		87.76

		2665		87.76

		2664		87.76

		2663		87.76

		2662		87.76

		2661		87.75

		2660		87.75

		2659		87.75

		2658		87.75

		2657		87.74

		2656		87.74

		2655		87.74

		2654		87.74

		2653		87.74

		2652		87.74

		2651		87.75

		2650		87.75

		2649		87.76

		2648		87.77

		2647		87.78

		2646		87.79

		2645		87.8

		2644		87.81

		2643		87.82

		2642		87.84

		2641		87.85

		2640		87.86

		2639		87.86

		2638		87.87

		2637		87.87

		2636		87.88

		2635		87.88

		2634		87.89

		2633		87.89

		2632		87.9

		2631		87.91

		2630		87.92

		2629		87.93

		2628		87.95

		2627		87.97

		2626		87.99

		2625		88.02

		2624		88.04

		2623		88.07

		2622		88.1

		2621		88.13

		2620		88.15

		2619		88.18

		2618		88.2

		2617		88.22

		2616		88.24

		2615		88.26

		2614		88.27

		2613		88.29

		2612		88.3

		2611		88.31

		2610		88.32

		2609		88.34

		2608		88.35

		2607		88.37

		2606		88.38

		2605		88.4

		2604		88.43

		2603		88.45

		2602		88.47

		2601		88.5

		2600		88.53

		2599		88.56

		2598		88.59

		2597		88.62

		2596		88.65

		2595		88.68

		2594		88.71

		2593		88.74

		2592		88.77

		2591		88.8

		2590		88.82

		2589		88.84

		2588		88.86

		2587		88.88

		2586		88.9

		2585		88.91

		2584		88.92

		2583		88.93

		2582		88.95

		2581		88.96

		2580		88.96

		2579		88.97

		2578		88.98

		2577		88.99

		2576		89

		2575		89.01

		2574		89.02

		2573		89.02

		2572		89.03

		2571		89.04

		2570		89.04

		2569		89.04

		2568		89.05

		2567		89.05

		2566		89.05

		2565		89.05

		2564		89.05

		2563		89.05

		2562		89.05

		2561		89.05

		2560		89.06

		2559		89.07

		2558		89.09

		2557		89.1

		2556		89.12

		2555		89.15

		2554		89.18

		2553		89.21

		2552		89.24

		2551		89.27

		2550		89.31

		2549		89.35

		2548		89.39

		2547		89.42

		2546		89.46

		2545		89.49

		2544		89.52

		2543		89.55

		2542		89.57

		2541		89.59

		2540		89.61

		2539		89.62

		2538		89.64

		2537		89.65

		2536		89.66

		2535		89.67

		2534		89.69

		2533		89.71

		2532		89.73

		2531		89.76

		2530		89.8

		2529		89.84

		2528		89.88

		2527		89.94

		2526		89.99

		2525		90.04

		2524		90.1

		2523		90.16

		2522		90.21

		2521		90.26

		2520		90.31

		2519		90.36

		2518		90.4

		2517		90.43

		2516		90.47

		2515		90.5

		2514		90.53

		2513		90.56

		2512		90.59

		2511		90.62

		2510		90.65

		2509		90.68

		2508		90.72

		2507		90.76

		2506		90.8

		2505		90.84

		2504		90.88

		2503		90.92

		2502		90.96

		2501		91

		2500		91.03

		2499		91.07

		2498		91.1

		2497		91.12

		2496		91.14

		2495		91.16

		2494		91.18

		2493		91.2

		2492		91.21

		2491		91.23

		2490		91.24

		2489		91.26

		2488		91.28

		2487		91.3

		2486		91.33

		2485		91.36

		2484		91.39

		2483		91.42

		2482		91.46

		2481		91.49

		2480		91.53

		2479		91.56

		2478		91.59

		2477		91.62

		2476		91.65

		2475		91.67

		2474		91.69

		2473		91.71

		2472		91.73

		2471		91.74

		2470		91.76

		2469		91.77

		2468		91.78

		2467		91.79

		2466		91.81

		2465		91.82

		2464		91.83

		2463		91.85

		2462		91.87

		2461		91.89

		2460		91.91

		2459		91.93

		2458		91.95

		2457		91.97

		2456		92

		2455		92.02

		2454		92.04

		2453		92.06

		2452		92.08

		2451		92.1

		2450		92.12

		2449		92.13

		2448		92.15

		2447		92.16

		2446		92.18

		2445		92.19

		2444		92.21

		2443		92.23

		2442		92.24

		2441		92.26

		2440		92.28

		2439		92.3

		2438		92.32

		2437		92.34

		2436		92.37

		2435		92.39

		2434		92.41

		2433		92.43

		2432		92.45

		2431		92.47

		2430		92.48

		2429		92.5

		2428		92.51

		2427		92.53

		2426		92.54

		2425		92.55

		2424		92.56

		2423		92.57

		2422		92.58

		2421		92.58

		2420		92.59

		2419		92.61

		2418		92.62

		2417		92.63

		2416		92.64

		2415		92.66

		2414		92.67

		2413		92.69

		2412		92.7

		2411		92.72

		2410		92.73

		2409		92.75

		2408		92.76

		2407		92.78

		2406		92.79

		2405		92.8

		2404		92.81

		2403		92.82

		2402		92.84

		2401		92.85

		2400		92.86

		2399		92.87

		2398		92.88

		2397		92.89

		2396		92.9

		2395		92.91

		2394		92.92

		2393		92.93

		2392		92.93

		2391		92.95

		2390		92.96

		2389		92.97

		2388		92.98

		2387		92.99

		2386		93.01

		2385		93.02

		2384		93.03

		2383		93.04

		2382		93.05

		2381		93.06

		2380		93.07

		2379		93.08

		2378		93.08

		2377		93.09

		2376		93.09

		2375		93.1

		2374		93.1

		2373		93.1

		2372		93.11

		2371		93.11

		2370		93.12

		2369		93.12

		2368		93.12

		2367		93.13

		2366		93.13

		2365		93.13

		2364		93.13

		2363		93.13

		2362		93.13

		2361		93.14

		2360		93.14

		2359		93.14

		2358		93.15

		2357		93.15

		2356		93.16

		2355		93.16

		2354		93.16

		2353		93.17

		2352		93.17

		2351		93.17

		2350		93.16

		2349		93.16

		2348		93.16

		2347		93.15

		2346		93.15

		2345		93.15

		2344		93.15

		2343		93.15

		2342		93.15

		2341		93.16

		2340		93.16

		2339		93.17

		2338		93.17

		2337		93.18

		2336		93.18

		2335		93.18

		2334		93.18

		2333		93.17

		2332		93.17

		2331		93.16

		2330		93.15

		2329		93.14

		2328		93.13

		2327		93.12

		2326		93.11

		2325		93.11

		2324		93.11

		2323		93.11

		2322		93.12

		2321		93.13

		2320		93.14

		2319		93.16

		2318		93.17

		2317		93.19

		2316		93.21

		2315		93.23

		2314		93.26

		2313		93.27

		2312		93.29

		2311		93.31

		2310		93.33

		2309		93.34

		2308		93.36

		2307		93.37

		2306		93.38

		2305		93.39

		2304		93.39

		2303		93.4

		2302		93.4

		2301		93.4

		2300		93.4

		2299		93.4

		2298		93.4

		2297		93.4

		2296		93.39

		2295		93.39

		2294		93.38

		2293		93.37

		2292		93.37

		2291		93.36

		2290		93.36

		2289		93.36

		2288		93.36

		2287		93.36

		2286		93.36

		2285		93.36

		2284		93.37

		2283		93.37

		2282		93.38

		2281		93.39

		2280		93.4

		2279		93.41

		2278		93.42

		2277		93.43

		2276		93.44

		2275		93.45

		2274		93.47

		2273		93.48

		2272		93.5

		2271		93.52

		2270		93.53

		2269		93.54

		2268		93.56

		2267		93.57

		2266		93.58

		2265		93.59

		2264		93.6

		2263		93.6

		2262		93.61

		2261		93.62

		2260		93.63

		2259		93.64

		2258		93.66

		2257		93.67

		2256		93.69

		2255		93.71

		2254		93.73

		2253		93.75

		2252		93.77

		2251		93.78

		2250		93.8

		2249		93.81

		2248		93.82

		2247		93.83

		2246		93.84

		2245		93.85

		2244		93.86

		2243		93.87

		2242		93.87

		2241		93.88

		2240		93.89

		2239		93.9

		2238		93.91

		2237		93.92

		2236		93.93

		2235		93.95

		2234		93.96

		2233		93.97

		2232		93.98

		2231		93.99

		2230		94

		2229		94.01

		2228		94.02

		2227		94.03

		2226		94.04

		2225		94.04

		2224		94.05

		2223		94.06

		2222		94.06

		2221		94.07

		2220		94.07

		2219		94.08

		2218		94.08

		2217		94.08

		2216		94.08

		2215		94.08

		2214		94.08

		2213		94.09

		2212		94.09

		2211		94.1

		2210		94.1

		2209		94.11

		2208		94.11

		2207		94.12

		2206		94.12

		2205		94.13

		2204		94.12

		2203		94.12

		2202		94.11

		2201		94.11

		2200		94.1

		2199		94.09

		2198		94.09

		2197		94.08

		2196		94.08

		2195		94.07

		2194		94.08

		2193		94.08

		2192		94.09

		2191		94.1

		2190		94.11

		2189		94.12

		2188		94.14

		2187		94.15

		2186		94.17

		2185		94.18

		2184		94.2

		2183		94.21

		2182		94.22

		2181		94.23

		2180		94.23

		2179		94.23

		2178		94.23

		2177		94.22

		2176		94.21

		2175		94.2

		2174		94.18

		2173		94.16

		2172		94.14

		2171		94.12

		2170		94.1

		2169		94.09

		2168		94.09

		2167		94.09

		2166		94.11

		2165		94.14

		2164		94.18

		2163		94.23

		2162		94.29

		2161		94.35

		2160		94.41

		2159		94.47

		2158		94.52

		2157		94.56

		2156		94.59

		2155		94.61

		2154		94.61

		2153		94.62

		2152		94.61

		2151		94.6

		2150		94.59

		2149		94.58

		2148		94.58

		2147		94.58

		2146		94.58

		2145		94.58

		2144		94.59

		2143		94.6

		2142		94.6

		2141		94.61

		2140		94.61

		2139		94.61

		2138		94.61

		2137		94.61

		2136		94.61

		2135		94.6

		2134		94.6

		2133		94.59

		2132		94.57

		2131		94.56

		2130		94.54

		2129		94.53

		2128		94.51

		2127		94.49

		2126		94.47

		2125		94.45

		2124		94.44

		2123		94.42

		2122		94.4

		2121		94.39

		2120		94.37

		2119		94.36

		2118		94.35

		2117		94.34

		2116		94.33

		2115		94.32

		2114		94.32

		2113		94.31

		2112		94.31

		2111		94.31

		2110		94.31

		2109		94.31

		2108		94.32

		2107		94.32

		2106		94.32

		2105		94.33

		2104		94.33

		2103		94.34

		2102		94.34

		2101		94.35

		2100		94.35

		2099		94.36

		2098		94.37

		2097		94.37

		2096		94.38

		2095		94.38

		2094		94.38

		2093		94.38

		2092		94.38

		2091		94.38

		2090		94.37

		2089		94.37

		2088		94.36

		2087		94.35

		2086		94.34

		2085		94.33

		2084		94.33

		2083		94.32

		2082		94.31

		2081		94.31

		2080		94.3

		2079		94.3

		2078		94.31

		2077		94.31

		2076		94.32

		2075		94.34

		2074		94.35

		2073		94.36

		2072		94.38

		2071		94.39

		2070		94.4

		2069		94.41

		2068		94.42

		2067		94.43

		2066		94.43

		2065		94.43

		2064		94.43

		2063		94.44

		2062		94.43

		2061		94.43

		2060		94.43

		2059		94.42

		2058		94.41

		2057		94.4

		2056		94.39

		2055		94.39

		2054		94.38

		2053		94.38

		2052		94.38

		2051		94.39

		2050		94.4

		2049		94.41

		2048		94.43

		2047		94.46

		2046		94.48

		2045		94.5

		2044		94.52

		2043		94.54

		2042		94.55

		2041		94.57

		2040		94.58

		2039		94.59

		2038		94.6

		2037		94.6

		2036		94.6

		2035		94.61

		2034		94.62

		2033		94.63

		2032		94.63

		2031		94.64

		2030		94.64

		2029		94.64

		2028		94.64

		2027		94.63

		2026		94.63

		2025		94.63

		2024		94.62

		2023		94.61

		2022		94.6

		2021		94.59

		2020		94.59

		2019		94.58

		2018		94.58

		2017		94.59

		2016		94.59

		2015		94.6

		2014		94.62

		2013		94.63

		2012		94.65

		2011		94.67

		2010		94.69

		2009		94.7

		2008		94.72

		2007		94.73

		2006		94.73

		2005		94.73

		2004		94.73

		2003		94.72

		2002		94.71

		2001		94.69

		2000		94.67

		1999		94.65

		1998		94.64

		1997		94.62

		1996		94.6

		1995		94.58

		1994		94.57

		1993		94.55

		1992		94.54

		1991		94.52

		1990		94.5

		1989		94.48

		1988		94.47

		1987		94.45

		1986		94.44

		1985		94.43

		1984		94.43

		1983		94.43

		1982		94.44

		1981		94.46

		1980		94.48

		1979		94.51

		1978		94.55

		1977		94.59

		1976		94.62

		1975		94.65

		1974		94.68

		1973		94.71

		1972		94.73

		1971		94.74

		1970		94.75

		1969		94.76

		1968		94.76

		1967		94.76

		1966		94.76

		1965		94.76

		1964		94.75

		1963		94.75

		1962		94.75

		1961		94.75

		1960		94.75

		1959		94.74

		1958		94.74

		1957		94.73

		1956		94.72

		1955		94.72

		1954		94.71

		1953		94.71

		1952		94.7

		1951		94.7

		1950		94.69

		1949		94.69

		1948		94.69

		1947		94.69

		1946		94.69

		1945		94.69

		1944		94.69

		1943		94.69

		1942		94.7

		1941		94.7

		1940		94.7

		1939		94.69

		1938		94.69

		1937		94.69

		1936		94.68

		1935		94.67

		1934		94.67

		1933		94.66

		1932		94.65

		1931		94.64

		1930		94.63

		1929		94.62

		1928		94.61

		1927		94.6

		1926		94.58

		1925		94.57

		1924		94.56

		1923		94.54

		1922		94.53

		1921		94.52

		1920		94.51

		1919		94.5

		1918		94.49

		1917		94.49

		1916		94.48

		1915		94.48

		1914		94.48

		1913		94.48

		1912		94.48

		1911		94.48

		1910		94.48

		1909		94.48

		1908		94.47

		1907		94.47

		1906		94.46

		1905		94.45

		1904		94.44

		1903		94.43

		1902		94.42

		1901		94.41

		1900		94.4

		1899		94.39

		1898		94.38

		1897		94.38

		1896		94.37

		1895		94.37

		1894		94.37

		1893		94.37

		1892		94.37

		1891		94.37

		1890		94.38

		1889		94.38

		1888		94.38

		1887		94.37

		1886		94.37

		1885		94.37

		1884		94.37

		1883		94.36

		1882		94.36

		1881		94.35

		1880		94.34

		1879		94.33

		1878		94.33

		1877		94.32

		1876		94.31

		1875		94.3

		1874		94.29

		1873		94.28

		1872		94.27

		1871		94.26

		1870		94.25

		1869		94.24

		1868		94.23

		1867		94.22

		1866		94.21

		1865		94.21

		1864		94.2

		1863		94.19

		1862		94.18

		1861		94.17

		1860		94.16

		1859		94.15

		1858		94.14

		1857		94.13

		1856		94.12

		1855		94.11

		1854		94.1

		1853		94.09

		1852		94.08

		1851		94.07

		1850		94.06

		1849		94.05

		1848		94.04

		1847		94.02

		1846		94.01

		1845		94

		1844		93.99

		1843		93.98

		1842		93.97

		1841		93.97

		1840		93.96

		1839		93.95

		1838		93.95

		1837		93.94

		1836		93.93

		1835		93.93

		1834		93.92

		1833		93.92

		1832		93.91

		1831		93.9

		1830		93.89

		1829		93.87

		1828		93.86

		1827		93.84

		1826		93.82

		1825		93.8

		1824		93.78

		1823		93.75

		1822		93.73

		1821		93.71

		1820		93.69

		1819		93.67

		1818		93.65

		1817		93.64

		1816		93.62

		1815		93.61

		1814		93.6

		1813		93.59

		1812		93.58

		1811		93.57

		1810		93.57

		1809		93.56

		1808		93.55

		1807		93.54

		1806		93.54

		1805		93.53

		1804		93.51

		1803		93.5

		1802		93.48

		1801		93.46

		1800		93.44

		1799		93.41

		1798		93.38

		1797		93.35

		1796		93.31

		1795		93.27

		1794		93.23

		1793		93.19

		1792		93.14

		1791		93.1

		1790		93.06

		1789		93.02

		1788		92.99

		1787		92.97

		1786		92.96

		1785		92.95

		1784		92.96

		1783		92.97

		1782		92.99

		1781		93.03

		1780		93.06

		1779		93.1

		1778		93.15

		1777		93.2

		1776		93.24

		1775		93.29

		1774		93.34

		1773		93.38

		1772		93.42

		1771		93.45

		1770		93.49

		1769		93.52

		1768		93.55

		1767		93.58

		1766		93.61

		1765		93.63

		1764		93.66

		1763		93.68

		1762		93.7

		1761		93.72

		1760		93.74

		1759		93.76

		1758		93.77

		1757		93.78

		1756		93.79

		1755		93.8

		1754		93.8

		1753		93.8

		1752		93.8

		1751		93.79

		1750		93.79

		1749		93.77

		1748		93.75

		1747		93.73

		1746		93.7

		1745		93.66

		1744		93.62

		1743		93.56

		1742		93.5

		1741		93.43

		1740		93.34

		1739		93.25

		1738		93.14

		1737		93.02

		1736		92.88

		1735		92.71

		1734		92.53

		1733		92.33

		1732		92.1

		1731		91.83

		1730		91.54

		1729		91.2

		1728		90.81

		1727		90.36

		1726		89.85

		1725		89.24

		1724		88.55

		1723		87.76

		1722		86.88

		1721		85.89

		1720		84.8

		1719		83.59

		1718		82.29

		1717		80.9

		1716		79.42

		1715		77.88

		1714		76.26

		1713		74.58

		1712		72.84

		1711		71.05

		1710		69.22

		1709		67.37

		1708		65.5

		1707		63.64

		1706		61.81

		1705		60.05

		1704		58.4

		1703		56.89

		1702		55.52

		1701		54.33

		1700		53.32

		1699		52.53

		1698		51.94

		1697		51.56

		1696		51.35

		1695		51.3

		1694		51.38

		1693		51.57

		1692		51.88

		1691		52.28

		1690		52.79

		1689		53.39

		1688		54.1

		1687		54.91

		1686		55.85

		1685		56.93

		1684		58.16

		1683		59.54

		1682		61.04

		1681		62.66

		1680		64.36

		1679		66.13

		1678		67.94

		1677		69.76

		1676		71.56

		1675		73.29

		1674		74.94

		1673		76.49

		1672		77.92

		1671		79.23

		1670		80.43

		1669		81.52

		1668		82.48

		1667		83.34

		1666		84.1

		1665		84.77

		1664		85.37

		1663		85.91

		1662		86.39

		1661		86.82

		1660		87.21

		1659		87.55

		1658		87.87

		1657		88.16

		1656		88.43

		1655		88.67

		1654		88.9

		1653		89.11

		1652		89.3

		1651		89.48

		1650		89.65

		1649		89.81

		1648		89.96

		1647		90.11

		1646		90.25

		1645		90.38

		1644		90.51

		1643		90.63

		1642		90.75

		1641		90.87

		1640		90.98

		1639		91.09

		1638		91.19

		1637		91.29

		1636		91.39

		1635		91.49

		1634		91.58

		1633		91.66

		1632		91.75

		1631		91.83

		1630		91.91

		1629		91.99

		1628		92.06

		1627		92.14

		1626		92.21

		1625		92.28

		1624		92.35

		1623		92.42

		1622		92.49

		1621		92.55

		1620		92.62

		1619		92.68

		1618		92.74

		1617		92.8

		1616		92.86

		1615		92.92

		1614		92.97

		1613		93.02

		1612		93.07

		1611		93.12

		1610		93.17

		1609		93.21

		1608		93.26

		1607		93.3

		1606		93.33

		1605		93.37

		1604		93.4

		1603		93.43

		1602		93.45

		1601		93.48

		1600		93.5

		1599		93.52

		1598		93.54

		1597		93.56

		1596		93.58

		1595		93.59

		1594		93.61

		1593		93.63

		1592		93.65

		1591		93.67

		1590		93.68

		1589		93.7

		1588		93.72

		1587		93.74

		1586		93.76

		1585		93.78

		1584		93.8

		1583		93.82

		1582		93.83

		1581		93.85

		1580		93.86

		1579		93.88

		1578		93.89

		1577		93.9

		1576		93.91

		1575		93.91

		1574		93.92

		1573		93.93

		1572		93.93

		1571		93.94

		1570		93.95

		1569		93.96

		1568		93.96

		1567		93.97

		1566		93.98

		1565		94

		1564		94.01

		1563		94.02

		1562		94.03

		1561		94.05

		1560		94.06

		1559		94.07

		1558		94.09

		1557		94.1

		1556		94.11

		1555		94.12

		1554		94.13

		1553		94.14

		1552		94.15

		1551		94.17

		1550		94.18

		1549		94.19

		1548		94.19

		1547		94.2

		1546		94.21

		1545		94.22

		1544		94.23

		1543		94.24

		1542		94.25

		1541		94.25

		1540		94.26

		1539		94.27

		1538		94.28

		1537		94.29

		1536		94.29

		1535		94.3

		1534		94.31

		1533		94.31

		1532		94.31

		1531		94.32

		1530		94.32

		1529		94.31

		1528		94.31

		1527		94.31

		1526		94.3

		1525		94.29

		1524		94.29

		1523		94.28

		1522		94.27

		1521		94.27

		1520		94.26

		1519		94.25

		1518		94.24

		1517		94.24

		1516		94.23

		1515		94.23

		1514		94.22

		1513		94.21

		1512		94.21

		1511		94.2

		1510		94.2

		1509		94.2

		1508		94.19

		1507		94.19

		1506		94.19

		1505		94.18

		1504		94.18

		1503		94.17

		1502		94.17

		1501		94.16

		1500		94.15

		1499		94.14

		1498		94.13

		1497		94.11

		1496		94.1

		1495		94.08

		1494		94.06

		1493		94.04

		1492		94.01

		1491		93.99

		1490		93.95

		1489		93.91

		1488		93.85

		1487		93.78

		1486		93.68

		1485		93.54

		1484		93.34

		1483		93.04

		1482		92.61

		1481		92.02

		1480		91.27

		1479		90.38

		1478		89.38

		1477		88.3

		1476		87.15

		1475		85.97

		1474		84.79

		1473		83.68

		1472		82.72

		1471		81.97

		1470		81.45

		1469		81.13

		1468		80.98

		1467		80.95

		1466		81.03

		1465		81.22

		1464		81.52

		1463		81.9

		1462		82.32

		1461		82.75

		1460		83.15

		1459		83.55

		1458		83.93

		1457		84.33

		1456		84.72

		1455		85.1

		1454		85.44

		1453		85.72

		1452		85.95

		1451		86.11

		1450		86.21

		1449		86.25

		1448		86.22

		1447		86.14

		1446		86

		1445		85.81

		1444		85.56

		1443		85.26

		1442		84.91

		1441		84.5

		1440		84.05

		1439		83.55

		1438		83.01

		1437		82.45

		1436		81.87

		1435		81.32

		1434		80.8

		1433		80.34

		1432		79.97

		1431		79.7

		1430		79.56

		1429		79.54

		1428		79.67

		1427		79.91

		1426		80.26

		1425		80.68

		1424		81.14

		1423		81.61

		1422		82.04

		1421		82.39

		1420		82.65

		1419		82.79

		1418		82.82

		1417		82.74

		1416		82.56

		1415		82.32

		1414		82.05

		1413		81.79

		1412		81.6

		1411		81.51

		1410		81.54

		1409		81.72

		1408		82.04

		1407		82.5

		1406		83.08

		1405		83.76

		1404		84.51

		1403		85.29

		1402		86.07

		1401		86.83

		1400		87.53

		1399		88.17

		1398		88.74

		1397		89.24

		1396		89.66

		1395		90.02

		1394		90.32

		1393		90.57

		1392		90.78

		1391		90.96

		1390		91.1

		1389		91.2

		1388		91.28

		1387		91.33

		1386		91.36

		1385		91.37

		1384		91.35

		1383		91.31

		1382		91.24

		1381		91.16

		1380		91.07

		1379		90.98

		1378		90.88

		1377		90.78

		1376		90.69

		1375		90.61

		1374		90.54

		1373		90.48

		1372		90.44

		1371		90.4

		1370		90.35

		1369		90.3

		1368		90.24

		1367		90.15

		1366		90.03

		1365		89.89

		1364		89.73

		1363		89.54

		1362		89.33

		1361		89.11

		1360		88.88

		1359		88.65

		1358		88.43

		1357		88.22

		1356		88.04

		1355		87.89

		1354		87.77

		1353		87.68

		1352		87.64

		1351		87.64

		1350		87.7

		1349		87.81

		1348		87.97

		1347		88.17

		1346		88.41

		1345		88.67

		1344		88.94

		1343		89.19

		1342		89.42

		1341		89.59

		1340		89.69

		1339		89.7

		1338		89.63

		1337		89.47

		1336		89.24

		1335		88.95

		1334		88.62

		1333		88.27

		1332		87.94

		1331		87.65

		1330		87.43

		1329		87.29

		1328		87.23

		1327		87.25

		1326		87.33

		1325		87.44

		1324		87.56

		1323		87.65

		1322		87.68

		1321		87.61

		1320		87.4

		1319		87.04

		1318		86.51

		1317		85.83

		1316		85

		1315		84.06

		1314		83.03

		1313		81.95

		1312		80.88

		1311		79.85

		1310		78.91

		1309		78.11

		1308		77.46

		1307		76.97

		1306		76.64

		1305		76.46

		1304		76.41

		1303		76.44

		1302		76.53

		1301		76.65

		1300		76.76

		1299		76.83

		1298		76.83

		1297		76.72

		1296		76.51

		1295		76.21

		1294		75.82

		1293		75.39

		1292		74.95

		1291		74.52

		1290		74.15

		1289		73.86

		1288		73.7

		1287		73.72

		1286		73.94

		1285		74.38

		1284		75.02

		1283		75.85

		1282		76.81

		1281		77.88

		1280		79.01

		1279		80.17

		1278		81.29

		1277		82.34

		1276		83.28

		1275		84.07

		1274		84.68

		1273		85.1

		1272		85.31

		1271		85.33

		1270		85.17

		1269		84.86

		1268		84.43

		1267		83.92

		1266		83.38

		1265		82.85

		1264		82.38

		1263		82.05

		1262		81.88

		1261		81.91

		1260		82.14

		1259		82.55

		1258		83.12

		1257		83.81

		1256		84.58

		1255		85.39

		1254		86.19

		1253		86.93

		1252		87.59

		1251		88.11

		1250		88.49

		1249		88.69

		1248		88.69

		1247		88.5

		1246		88.11

		1245		87.55

		1244		86.84

		1243		86.02

		1242		85.13

		1241		84.21

		1240		83.34

		1239		82.57

		1238		81.99

		1237		81.64

		1236		81.54

		1235		81.7

		1234		82.08

		1233		82.66

		1232		83.38

		1231		84.2

		1230		85.06

		1229		85.9

		1228		86.67

		1227		87.32

		1226		87.81

		1225		88.13

		1224		88.25

		1223		88.2

		1222		87.97

		1221		87.6

		1220		87.11

		1219		86.52

		1218		85.87

		1217		85.19

		1216		84.54

		1215		83.97

		1214		83.53

		1213		83.26

		1212		83.18

		1211		83.28

		1210		83.57

		1209		84.01

		1208		84.59

		1207		85.28

		1206		86.03

		1205		86.79

		1204		87.5

		1203		88.12

		1202		88.59

		1201		88.88

		1200		88.98

		1199		88.88

		1198		88.61

		1197		88.18

		1196		87.65

		1195		87.04

		1194		86.42

		1193		85.83

		1192		85.34

		1191		85.01

		1190		84.89

		1189		84.98

		1188		85.27

		1187		85.74

		1186		86.34

		1185		87.03

		1184		87.77

		1183		88.53

		1182		89.26

		1181		89.94

		1180		90.53

		1179		91.03

		1178		91.43

		1177		91.76

		1176		92.02

		1175		92.24

		1174		92.42

		1173		92.58

		1172		92.71

		1171		92.83

		1170		92.93

		1169		93.03

		1168		93.11

		1167		93.18

		1166		93.25

		1165		93.31

		1164		93.37

		1163		93.42

		1162		93.47

		1161		93.52

		1160		93.56

		1159		93.6

		1158		93.64

		1157		93.67

		1156		93.7

		1155		93.73

		1154		93.76

		1153		93.79

		1152		93.81

		1151		93.83

		1150		93.85

		1149		93.87

		1148		93.89

		1147		93.9

		1146		93.92

		1145		93.93

		1144		93.94

		1143		93.95

		1142		93.96

		1141		93.96

		1140		93.96

		1139		93.95

		1138		93.94

		1137		93.91

		1136		93.87

		1135		93.82

		1134		93.75

		1133		93.66

		1132		93.56

		1131		93.43

		1130		93.3

		1129		93.17

		1128		93.04

		1127		92.92

		1126		92.81

		1125		92.73

		1124		92.67

		1123		92.65

		1122		92.65

		1121		92.69

		1120		92.74

		1119		92.82

		1118		92.89

		1117		92.97

		1116		93.05

		1115		93.11

		1114		93.17

		1113		93.21

		1112		93.23

		1111		93.25

		1110		93.26

		1109		93.26

		1108		93.25

		1107		93.24

		1106		93.21

		1105		93.16

		1104		93.08

		1103		92.94

		1102		92.75

		1101		92.5

		1100		92.2

		1099		91.85

		1098		91.47

		1097		91.07

		1096		90.68

		1095		90.31

		1094		89.99

		1093		89.76

		1092		89.63

		1091		89.59

		1090		89.66

		1089		89.8

		1088		90

		1087		90.24

		1086		90.49

		1085		90.75

		1084		90.99

		1083		91.2

		1082		91.37

		1081		91.5

		1080		91.58

		1079		91.63

		1078		91.66

		1077		91.67

		1076		91.66

		1075		91.64

		1074		91.62

		1073		91.58

		1072		91.55

		1071		91.5

		1070		91.45

		1069		91.4

		1068		91.34

		1067		91.29

		1066		91.23

		1065		91.18

		1064		91.14

		1063		91.09

		1062		91.05

		1061		91.01

		1060		90.97

		1059		90.93

		1058		90.9

		1057		90.87

		1056		90.86

		1055		90.84

		1054		90.84

		1053		90.85

		1052		90.86

		1051		90.89

		1050		90.92

		1049		90.96

		1048		90.99

		1047		91.03

		1046		91.06

		1045		91.08

		1044		91.09

		1043		91.09

		1042		91.08

		1041		91.07

		1040		91.06

		1039		91.06

		1038		91.07

		1037		91.09

		1036		91.13

		1035		91.17

		1034		91.23

		1033		91.3

		1032		91.4

		1031		91.49

		1030		91.59

		1029		91.67

		1028		91.75

		1027		91.81

		1026		91.86

		1025		91.9

		1024		91.93

		1023		91.94

		1022		91.94

		1021		91.94

		1020		91.93

		1019		91.92

		1018		91.91

		1017		91.89

		1016		91.88

		1015		91.87

		1014		91.85

		1013		91.83

		1012		91.81

		1011		91.79

		1010		91.76

		1009		91.73

		1008		91.69

		1007		91.64

		1006		91.6

		1005		91.55

		1004		91.51

		1003		91.47

		1002		91.44

		1001		91.42

		1000		91.41

		999		91.42

		998		91.43

		997		91.46

		996		91.49

		995		91.52

		994		91.54

		993		91.54

		992		91.54

		991		91.53

		990		91.5

		989		91.45

		988		91.4

		987		91.34

		986		91.27

		985		91.2

		984		91.14

		983		91.07

		982		90.99

		981		90.9

		980		90.8

		979		90.67

		978		90.52

		977		90.34

		976		90.13

		975		89.89

		974		89.61

		973		89.3

		972		88.95

		971		88.58

		970		88.19

		969		87.78

		968		87.36

		967		86.93

		966		86.49

		965		86.04

		964		85.59

		963		85.14

		962		84.68

		961		84.23

		960		83.78

		959		83.33

		958		82.87

		957		82.41

		956		81.94

		955		81.46

		954		80.97

		953		80.47

		952		79.95

		951		79.41

		950		78.85

		949		78.28

		948		77.7

		947		77.11

		946		76.53

		945		75.98

		944		75.45

		943		74.98

		942		74.56

		941		74.23

		940		73.99

		939		73.85

		938		73.81

		937		73.88

		936		74.06

		935		74.34

		934		74.72

		933		75.18

		932		75.72

		931		76.31

		930		76.95

		929		77.62

		928		78.31

		927		79.01

		926		79.7

		925		80.37

		924		81

		923		81.6

		922		82.15

		921		82.65

		920		83.09

		919		83.46

		918		83.76

		917		84

		916		84.17

		915		84.29

		914		84.37

		913		84.41

		912		84.44

		911		84.47

		910		84.52

		909		84.58

		908		84.68

		907		84.81

		906		84.97

		905		85.17

		904		85.38

		903		85.59

		902		85.78

		901		85.95

		900		86.09

		899		86.18

		898		86.22

		897		86.21

		896		86.17

		895		86.09

		894		86

		893		85.9

		892		85.82

		891		85.77

		890		85.75

		889		85.78

		888		85.85

		887		85.98

		886		86.15

		885		86.37

		884		86.61

		883		86.88

		882		87.15

		881		87.42

		880		87.69

		879		87.95

		878		88.2

		877		88.43

		876		88.64

		875		88.83

		874		89.01

		873		89.17

		872		89.33

		871		89.48

		870		89.62

		869		89.76

		868		89.89

		867		90.02

		866		90.14

		865		90.26

		864		90.38

		863		90.5

		862		90.62

		861		90.75

		860		90.87

		859		91

		858		91.13

		857		91.27

		856		91.4

		855		91.54

		854		91.67

		853		91.8

		852		91.92

		851		92.04

		850		92.16

		849		92.26

		848		92.36

		847		92.46

		846		92.54

		845		92.63

		844		92.7

		843		92.78

		842		92.85

		841		92.91

		840		92.98

		839		93.04

		838		93.09

		837		93.15

		836		93.2

		835		93.24

		834		93.29

		833		93.33

		832		93.36

		831		93.39

		830		93.41

		829		93.42

		828		93.42

		827		93.4

		826		93.35

		825		93.27

		824		93.16

		823		93.01

		822		92.83

		821		92.64

		820		92.45

		819		92.26

		818		92.09

		817		91.94

		816		91.85

		815		91.82

		814		91.87

		813		91.99

		812		92.16

		811		92.39

		810		92.64

		809		92.9

		808		93.16

		807		93.41

		806		93.64

		805		93.85

		804		94.01

		803		94.15

		802		94.24

		801		94.32

		800		94.37

		799		94.42

		798		94.45

		797		94.48

		796		94.5

		795		94.52

		794		94.52

		793		94.52

		792		94.49

		791		94.46

		790		94.4

		789		94.33

		788		94.25

		787		94.16

		786		94.08

		785		93.99

		784		93.92

		783		93.86

		782		93.83

		781		93.83

		780		93.86

		779		93.92

		778		94

		777		94.09

		776		94.2

		775		94.3

		774		94.4

		773		94.49

		772		94.57

		771		94.64

		770		94.68

		769		94.71

		768		94.72

		767		94.71

		766		94.68

		765		94.62

		764		94.53

		763		94.4

		762		94.21

		761		93.99

		760		93.73

		759		93.46

		758		93.18

		757		92.91

		756		92.66

		755		92.46

		754		92.32

		753		92.26

		752		92.29

		751		92.41

		750		92.59

		749		92.82

		748		93.06

		747		93.31

		746		93.53

		745		93.72

		744		93.85

		743		93.92

		742		93.91

		741		93.81

		740		93.61

		739		93.29

		738		92.84

		737		92.25

		736		91.51

		735		90.65

		734		89.67

		733		88.59

		732		87.44

		731		86.23

		730		84.99

		729		83.77

		728		82.63

		727		81.65

		726		80.88

		725		80.32

		724		80

		723		79.88

		722		79.99

		721		80.32

		720		80.89

		719		81.69

		718		82.66

		717		83.74

		716		84.86

		715		85.98

		714		87.06

		713		88.08

		712		89.02

		711		89.85

		710		90.56

		709		91.12

		708		91.54

		707		91.84

		706		92.02

		705		92.12

		704		92.14

		703		92.08

		702		91.96

		701		91.76

		700		91.48

		699		91.13

		698		90.7

		697		90.2

		696		89.64

		695		89.03

		694		88.39

		693		87.74

		692		87.12

		691		86.53

		690		86.02

		689		85.6

		688		85.29

		687		85.1

		686		85.02

		685		85.05

		684		85.18

		683		85.39

		682		85.66

		681		85.97

		680		86.3

		679		86.63

		678		86.96

		677		87.27

		676		87.56

		675		87.83

		674		88.08

		673		88.32

		672		88.54

		671		88.77

		670		88.99

		669		89.21

		668		89.44

		667		89.68

		666		89.92

		665		90.17

		664		90.43

		663		90.69

		662		90.95

		661		91.2

		660		91.46

		659		91.7

		658		91.93

		657		92.15

		656		92.36

		655		92.55

		654		92.73

		653		92.88

		652		93.02

		651		93.15

		650		93.25

		649		93.34

		648		93.42

		647		93.47

		646		93.51

		645		93.54

		644		93.56

		643		93.56

		642		93.57

		641		93.56

		640		93.56

		639		93.57

		638		93.57

		637		93.59

		636		93.62

		635		93.65

		634		93.7

		633		93.75

		632		93.81

		631		93.87

		630		93.94

		629		94.01

		628		94.07

		627		94.14

		626		94.19

		625		94.24

		624		94.29

		623		94.33

		622		94.37

		621		94.4

		620		94.43

		619		94.45

		618		94.47

		617		94.49

		616		94.5

		615		94.52

		614		94.53

		613		94.55

		612		94.57

		611		94.58

		610		94.6

		609		94.61

		608		94.62

		607		94.64

		606		94.65

		605		94.66

		604		94.67

		603		94.68

		602		94.68

		601		94.69

		600		94.7

		599		94.71

		598		94.72

		597		94.72

		596		94.73

		595		94.74

		594		94.75

		593		94.76

		592		94.76

		591		94.76

		590		94.76

		589		94.76

		588		94.76

		587		94.75

		586		94.74

		585		94.72

		584		94.7

		583		94.67

		582		94.64

		581		94.6

		580		94.54

		579		94.48

		578		94.4

		577		94.31

		576		94.2

		575		94.08

		574		93.95

		573		93.79

		572		93.63

		571		93.44

		570		93.23

		569		93.01

		568		92.76

		567		92.5

		566		92.22

		565		91.92

		564		91.59

		563		91.24

		562		90.86

		561		90.47

		560		90.05

		559		89.61

		558		89.16

		557		88.7

		556		88.23

		555		87.78

		554		87.35

		553		86.95

		552		86.61

		551		86.33

		550		86.13

		549		86.02

		548		86.01

		547		86.1

		546		86.3

		545		86.6

		544		86.99

		543		87.45

		542		87.98

		541		88.54

		540		89.12

		539		89.71

		538		90.28

		537		90.82

		536		91.32

		535		91.78

		534		92.19

		533		92.55

		532		92.86

		531		93.13

		530		93.35

		529		93.54

		528		93.7

		527		93.83

		526		93.95

		525		94.04

		524		94.13

		523		94.2

		522		94.26

		521		94.32

		520		94.37

		519		94.42

		518		94.46

		517		94.49

		516		94.5

		515		94.5

		514		94.48

		513		94.43

		512		94.34

		511		94.2

		510		93.99

		509		93.72

		508		93.39

		507		93

		506		92.57

		505		92.11

		504		91.64

		503		91.18

		502		90.78

		501		90.44

		500		90.21

		499		90.09

		498		90.09

		497		90.2

		496		90.4

		495		90.69

		494		91.03

		493		91.4

		492		91.78

		491		92.15

		490		92.49

		489		92.78

		488		93.03

		487		93.23

		486		93.39

		485		93.52

		484		93.62

		483		93.71

		482		93.78

		481		93.85

		480		93.92

		479		93.99

		478		94.05

		477		94.12

		476		94.18

		475		94.25

		474		94.31

		473		94.37

		472		94.43

		471		94.49

		470		94.54

		469		94.58

		468		94.62

		467		94.65

		466		94.68

		465		94.71

		464		94.72

		463		94.73

		462		94.73

		461		94.72

		460		94.71

		459		94.68

		458		94.65

		457		94.62

		456		94.57

		455		94.51

		454		94.43

		453		94.34

		452		94.24

		451		94.11

		450		93.95

		449		93.76

		448		93.51

		447		93.21

		446		92.84

		445		92.41

		444		91.92

		443		91.39

		442		90.84

		441		90.29

		440		89.77

		439		89.31

		438		88.93

		437		88.67

		436		88.54

		435		88.57

		434		88.74

		433		89.04

		432		89.44

		431		89.91

		430		90.43

		429		90.97

		428		91.5

		427		91.99

		426		92.43

		425		92.79

		424		93.07

		423		93.27

		422		93.4

		421		93.46

		420		93.48

		419		93.47

		418		93.44

		417		93.4

		416		93.37

		415		93.35

		414		93.37

		413		93.43

		412		93.52

		411		93.64

		410		93.79

		409		93.95

		408		94.12

		407		94.27

		406		94.4

		405		94.49

		404		94.55

		403		94.56

		402		94.54

		401		94.49

		400		94.43
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		cm-1		%T

		4000		93.76

		3999		93.76

		3998		93.76

		3997		93.76

		3996		93.77

		3995		93.77

		3994		93.76

		3993		93.76

		3992		93.76

		3991		93.76

		3990		93.76

		3989		93.76

		3988		93.76

		3987		93.76

		3986		93.76

		3985		93.75

		3984		93.75

		3983		93.75

		3982		93.75

		3981		93.75

		3980		93.75

		3979		93.75

		3978		93.75

		3977		93.75

		3976		93.75

		3975		93.75

		3974		93.75

		3973		93.76

		3972		93.76

		3971		93.76

		3970		93.76

		3969		93.76

		3968		93.76

		3967		93.76

		3966		93.76

		3965		93.76

		3964		93.76

		3963		93.76

		3962		93.76

		3961		93.76

		3960		93.76

		3959		93.76

		3958		93.76

		3957		93.76

		3956		93.76

		3955		93.76

		3954		93.76

		3953		93.76

		3952		93.76

		3951		93.75

		3950		93.75

		3949		93.75

		3948		93.75

		3947		93.75

		3946		93.75

		3945		93.75

		3944		93.75

		3943		93.75

		3942		93.75

		3941		93.75

		3940		93.75

		3939		93.75

		3938		93.75

		3937		93.75

		3936		93.75

		3935		93.75

		3934		93.75

		3933		93.75

		3932		93.75

		3931		93.76

		3930		93.76

		3929		93.76

		3928		93.75

		3927		93.75

		3926		93.75

		3925		93.75

		3924		93.75

		3923		93.74

		3922		93.74

		3921		93.73

		3920		93.73

		3919		93.72

		3918		93.72

		3917		93.72

		3916		93.72

		3915		93.72

		3914		93.72

		3913		93.71

		3912		93.71

		3911		93.71

		3910		93.71

		3909		93.71

		3908		93.71

		3907		93.71

		3906		93.71

		3905		93.71

		3904		93.7

		3903		93.7

		3902		93.7

		3901		93.7

		3900		93.7

		3899		93.7

		3898		93.7

		3897		93.7

		3896		93.7

		3895		93.7

		3894		93.7

		3893		93.7

		3892		93.7

		3891		93.7

		3890		93.7

		3889		93.69

		3888		93.69

		3887		93.69

		3886		93.69

		3885		93.69

		3884		93.69

		3883		93.69

		3882		93.69

		3881		93.69

		3880		93.69

		3879		93.69

		3878		93.69

		3877		93.69

		3876		93.69

		3875		93.69

		3874		93.68

		3873		93.68

		3872		93.68

		3871		93.68

		3870		93.68

		3869		93.68

		3868		93.68

		3867		93.68

		3866		93.68

		3865		93.68

		3864		93.68

		3863		93.68

		3862		93.69

		3861		93.69

		3860		93.69

		3859		93.69

		3858		93.69

		3857		93.69

		3856		93.69

		3855		93.69

		3854		93.69

		3853		93.69

		3852		93.69

		3851		93.69

		3850		93.69

		3849		93.69

		3848		93.69

		3847		93.69

		3846		93.69

		3845		93.69

		3844		93.68

		3843		93.68

		3842		93.68

		3841		93.68

		3840		93.67

		3839		93.67

		3838		93.67

		3837		93.67

		3836		93.67

		3835		93.67

		3834		93.67

		3833		93.67

		3832		93.67

		3831		93.68

		3830		93.68

		3829		93.68

		3828		93.68

		3827		93.68

		3826		93.68

		3825		93.68

		3824		93.68

		3823		93.68

		3822		93.69

		3821		93.69

		3820		93.69

		3819		93.69

		3818		93.69

		3817		93.69

		3816		93.69

		3815		93.7

		3814		93.7

		3813		93.7

		3812		93.7

		3811		93.7

		3810		93.7

		3809		93.69

		3808		93.69

		3807		93.69

		3806		93.69

		3805		93.69

		3804		93.69

		3803		93.69

		3802		93.69

		3801		93.69

		3800		93.7

		3799		93.7

		3798		93.71

		3797		93.71

		3796		93.71

		3795		93.72

		3794		93.72

		3793		93.72

		3792		93.73

		3791		93.73

		3790		93.73

		3789		93.73

		3788		93.73

		3787		93.74

		3786		93.74

		3785		93.74

		3784		93.74

		3783		93.74

		3782		93.74

		3781		93.75

		3780		93.75

		3779		93.75

		3778		93.75

		3777		93.75

		3776		93.75

		3775		93.75

		3774		93.75

		3773		93.75

		3772		93.74

		3771		93.74

		3770		93.74

		3769		93.74

		3768		93.74

		3767		93.74

		3766		93.74

		3765		93.74

		3764		93.73

		3763		93.73

		3762		93.73

		3761		93.73

		3760		93.72

		3759		93.72

		3758		93.71

		3757		93.7

		3756		93.7

		3755		93.69

		3754		93.68

		3753		93.68

		3752		93.67

		3751		93.67

		3750		93.67

		3749		93.67

		3748		93.67

		3747		93.67

		3746		93.67

		3745		93.67

		3744		93.67

		3743		93.68

		3742		93.68

		3741		93.68

		3740		93.68

		3739		93.69

		3738		93.69

		3737		93.69

		3736		93.69

		3735		93.69

		3734		93.69

		3733		93.69

		3732		93.69

		3731		93.69

		3730		93.69

		3729		93.69

		3728		93.69

		3727		93.69

		3726		93.69

		3725		93.69

		3724		93.68

		3723		93.68

		3722		93.67

		3721		93.67

		3720		93.66

		3719		93.65

		3718		93.64

		3717		93.63

		3716		93.62

		3715		93.61

		3714		93.6

		3713		93.59

		3712		93.58

		3711		93.57

		3710		93.56

		3709		93.55

		3708		93.54

		3707		93.53

		3706		93.52

		3705		93.51

		3704		93.49

		3703		93.48

		3702		93.47

		3701		93.45

		3700		93.43

		3699		93.42

		3698		93.4

		3697		93.38

		3696		93.36

		3695		93.35

		3694		93.33

		3693		93.32

		3692		93.3

		3691		93.29

		3690		93.28

		3689		93.27

		3688		93.25

		3687		93.24

		3686		93.23

		3685		93.22

		3684		93.21

		3683		93.2

		3682		93.19

		3681		93.18

		3680		93.16

		3679		93.15

		3678		93.14

		3677		93.13

		3676		93.12

		3675		93.11

		3674		93.1

		3673		93.1

		3672		93.09

		3671		93.09

		3670		93.09

		3669		93.09

		3668		93.1

		3667		93.1

		3666		93.1

		3665		93.11

		3664		93.11

		3663		93.12

		3662		93.13

		3661		93.13

		3660		93.14

		3659		93.15

		3658		93.16

		3657		93.17

		3656		93.19

		3655		93.2

		3654		93.22

		3653		93.24

		3652		93.25

		3651		93.27

		3650		93.29

		3649		93.31

		3648		93.33

		3647		93.35

		3646		93.37

		3645		93.39

		3644		93.41

		3643		93.43

		3642		93.45

		3641		93.47

		3640		93.49

		3639		93.5

		3638		93.52

		3637		93.53

		3636		93.54

		3635		93.56

		3634		93.57

		3633		93.57

		3632		93.58

		3631		93.59

		3630		93.6

		3629		93.61

		3628		93.62

		3627		93.63

		3626		93.63

		3625		93.64

		3624		93.65

		3623		93.66

		3622		93.66

		3621		93.67

		3620		93.67

		3619		93.67

		3618		93.67

		3617		93.66

		3616		93.66

		3615		93.65

		3614		93.65

		3613		93.64

		3612		93.64

		3611		93.63

		3610		93.63

		3609		93.63

		3608		93.63

		3607		93.63

		3606		93.64

		3605		93.64

		3604		93.65

		3603		93.66

		3602		93.66

		3601		93.67

		3600		93.68

		3599		93.69

		3598		93.69

		3597		93.7

		3596		93.71

		3595		93.71

		3594		93.72

		3593		93.72

		3592		93.73

		3591		93.73

		3590		93.74

		3589		93.74

		3588		93.74

		3587		93.75

		3586		93.75

		3585		93.75

		3584		93.75

		3583		93.76

		3582		93.76

		3581		93.76

		3580		93.76

		3579		93.76

		3578		93.76

		3577		93.76

		3576		93.76

		3575		93.76

		3574		93.76

		3573		93.76

		3572		93.76

		3571		93.76

		3570		93.76

		3569		93.76

		3568		93.76

		3567		93.76

		3566		93.76

		3565		93.75

		3564		93.75

		3563		93.75

		3562		93.75

		3561		93.75

		3560		93.75

		3559		93.75

		3558		93.75

		3557		93.75

		3556		93.75

		3555		93.75

		3554		93.75

		3553		93.75

		3552		93.75

		3551		93.75

		3550		93.75

		3549		93.75

		3548		93.75

		3547		93.74

		3546		93.74

		3545		93.74

		3544		93.74

		3543		93.74

		3542		93.74

		3541		93.74

		3540		93.74

		3539		93.74

		3538		93.74

		3537		93.74

		3536		93.74

		3535		93.74

		3534		93.74

		3533		93.74

		3532		93.74

		3531		93.74

		3530		93.74

		3529		93.74

		3528		93.74

		3527		93.74

		3526		93.74

		3525		93.74

		3524		93.74

		3523		93.74

		3522		93.74

		3521		93.74

		3520		93.74

		3519		93.74

		3518		93.74

		3517		93.74

		3516		93.74

		3515		93.74

		3514		93.74

		3513		93.74

		3512		93.74

		3511		93.74

		3510		93.74

		3509		93.74

		3508		93.74

		3507		93.74

		3506		93.74

		3505		93.74

		3504		93.74

		3503		93.74

		3502		93.74

		3501		93.74

		3500		93.74

		3499		93.74

		3498		93.74

		3497		93.73

		3496		93.73

		3495		93.73

		3494		93.73

		3493		93.73

		3492		93.73

		3491		93.73

		3490		93.73

		3489		93.73

		3488		93.73

		3487		93.73

		3486		93.73

		3485		93.73

		3484		93.73

		3483		93.73

		3482		93.73

		3481		93.73

		3480		93.72

		3479		93.72

		3478		93.72

		3477		93.72

		3476		93.72

		3475		93.72

		3474		93.72

		3473		93.72

		3472		93.72

		3471		93.72

		3470		93.73

		3469		93.73

		3468		93.73

		3467		93.73

		3466		93.73

		3465		93.73

		3464		93.72

		3463		93.72

		3462		93.72

		3461		93.72

		3460		93.71

		3459		93.71

		3458		93.71

		3457		93.7

		3456		93.7

		3455		93.7

		3454		93.7

		3453		93.7

		3452		93.7

		3451		93.69

		3450		93.69

		3449		93.69

		3448		93.69

		3447		93.69

		3446		93.69

		3445		93.69

		3444		93.69

		3443		93.69

		3442		93.69

		3441		93.69

		3440		93.69

		3439		93.69

		3438		93.69

		3437		93.69

		3436		93.68

		3435		93.68

		3434		93.67

		3433		93.67

		3432		93.66

		3431		93.65

		3430		93.64

		3429		93.63

		3428		93.62

		3427		93.61

		3426		93.6

		3425		93.59

		3424		93.58

		3423		93.58

		3422		93.57

		3421		93.57

		3420		93.56

		3419		93.56

		3418		93.56

		3417		93.56

		3416		93.56

		3415		93.56

		3414		93.56

		3413		93.55

		3412		93.55

		3411		93.55

		3410		93.55

		3409		93.55

		3408		93.55

		3407		93.56

		3406		93.56

		3405		93.56

		3404		93.56

		3403		93.57

		3402		93.57

		3401		93.57

		3400		93.57

		3399		93.57

		3398		93.57

		3397		93.56

		3396		93.56

		3395		93.55

		3394		93.54

		3393		93.53

		3392		93.52

		3391		93.51

		3390		93.5

		3389		93.48

		3388		93.47

		3387		93.46

		3386		93.45

		3385		93.44

		3384		93.44

		3383		93.44

		3382		93.43

		3381		93.43

		3380		93.44

		3379		93.44

		3378		93.45

		3377		93.45

		3376		93.46

		3375		93.47

		3374		93.48

		3373		93.48

		3372		93.49

		3371		93.49

		3370		93.49

		3369		93.49

		3368		93.49

		3367		93.49

		3366		93.48

		3365		93.47

		3364		93.46

		3363		93.45

		3362		93.44

		3361		93.43

		3360		93.42

		3359		93.41

		3358		93.41

		3357		93.4

		3356		93.4

		3355		93.4

		3354		93.4

		3353		93.4

		3352		93.4

		3351		93.4

		3350		93.4

		3349		93.39

		3348		93.39

		3347		93.39

		3346		93.38

		3345		93.38

		3344		93.38

		3343		93.37

		3342		93.37

		3341		93.36

		3340		93.36

		3339		93.35

		3338		93.34

		3337		93.34

		3336		93.33

		3335		93.32

		3334		93.32

		3333		93.31

		3332		93.3

		3331		93.3

		3330		93.29

		3329		93.29

		3328		93.28

		3327		93.28

		3326		93.28

		3325		93.27

		3324		93.27

		3323		93.27

		3322		93.26

		3321		93.26

		3320		93.26

		3319		93.26

		3318		93.26

		3317		93.26

		3316		93.26

		3315		93.26

		3314		93.26

		3313		93.26

		3312		93.26

		3311		93.27

		3310		93.27

		3309		93.27

		3308		93.27

		3307		93.27

		3306		93.26

		3305		93.26

		3304		93.25

		3303		93.25

		3302		93.24

		3301		93.23

		3300		93.23

		3299		93.22

		3298		93.21

		3297		93.2

		3296		93.2

		3295		93.19

		3294		93.18

		3293		93.17

		3292		93.16

		3291		93.15

		3290		93.14

		3289		93.13

		3288		93.12

		3287		93.11

		3286		93.1

		3285		93.09

		3284		93.08

		3283		93.08

		3282		93.07

		3281		93.06

		3280		93.06

		3279		93.05

		3278		93.04

		3277		93.04

		3276		93.03

		3275		93.02

		3274		93.02

		3273		93.01

		3272		93

		3271		92.99

		3270		92.97

		3269		92.96

		3268		92.95

		3267		92.94

		3266		92.93

		3265		92.91

		3264		92.9

		3263		92.89

		3262		92.88

		3261		92.87

		3260		92.86

		3259		92.85

		3258		92.84

		3257		92.83

		3256		92.81

		3255		92.8

		3254		92.79

		3253		92.78

		3252		92.77

		3251		92.76

		3250		92.74

		3249		92.73

		3248		92.72

		3247		92.71

		3246		92.69

		3245		92.68

		3244		92.66

		3243		92.65

		3242		92.64

		3241		92.62

		3240		92.61

		3239		92.6

		3238		92.58

		3237		92.57

		3236		92.55

		3235		92.54

		3234		92.52

		3233		92.51

		3232		92.49

		3231		92.47

		3230		92.46

		3229		92.44

		3228		92.42

		3227		92.41

		3226		92.39

		3225		92.38

		3224		92.36

		3223		92.34

		3222		92.33

		3221		92.31

		3220		92.3

		3219		92.28

		3218		92.26

		3217		92.25

		3216		92.23

		3215		92.22

		3214		92.2

		3213		92.18

		3212		92.17

		3211		92.15

		3210		92.14

		3209		92.12

		3208		92.1

		3207		92.08

		3206		92.07

		3205		92.05

		3204		92.03

		3203		92.02

		3202		92

		3201		91.98

		3200		91.97

		3199		91.95

		3198		91.94

		3197		91.92

		3196		91.91

		3195		91.89

		3194		91.88

		3193		91.86

		3192		91.85

		3191		91.84

		3190		91.82

		3189		91.81

		3188		91.79

		3187		91.77

		3186		91.76

		3185		91.74

		3184		91.73

		3183		91.71

		3182		91.7

		3181		91.68

		3180		91.67

		3179		91.65

		3178		91.64

		3177		91.63

		3176		91.61

		3175		91.6

		3174		91.59

		3173		91.57

		3172		91.55

		3171		91.54

		3170		91.52

		3169		91.5

		3168		91.49

		3167		91.47

		3166		91.45

		3165		91.43

		3164		91.41

		3163		91.39

		3162		91.37

		3161		91.36

		3160		91.34

		3159		91.32

		3158		91.3

		3157		91.28

		3156		91.27

		3155		91.25

		3154		91.23

		3153		91.2

		3152		91.18

		3151		91.16

		3150		91.14

		3149		91.11

		3148		91.09

		3147		91.07

		3146		91.04

		3145		91.01

		3144		90.99

		3143		90.96

		3142		90.94

		3141		90.91

		3140		90.88

		3139		90.85

		3138		90.83

		3137		90.8

		3136		90.77

		3135		90.74

		3134		90.71

		3133		90.68

		3132		90.65

		3131		90.62

		3130		90.6

		3129		90.57

		3128		90.54

		3127		90.51

		3126		90.48

		3125		90.46

		3124		90.43

		3123		90.4

		3122		90.37

		3121		90.34

		3120		90.32

		3119		90.29

		3118		90.26

		3117		90.23

		3116		90.2

		3115		90.17

		3114		90.14

		3113		90.11

		3112		90.08

		3111		90.05

		3110		90.02

		3109		89.99

		3108		89.96

		3107		89.93

		3106		89.9

		3105		89.87

		3104		89.84

		3103		89.81

		3102		89.78

		3101		89.76

		3100		89.73

		3099		89.7

		3098		89.68

		3097		89.65

		3096		89.63

		3095		89.61

		3094		89.59

		3093		89.56

		3092		89.54

		3091		89.52

		3090		89.5

		3089		89.48

		3088		89.46

		3087		89.45

		3086		89.43

		3085		89.41

		3084		89.39

		3083		89.37

		3082		89.35

		3081		89.33

		3080		89.31

		3079		89.29

		3078		89.26

		3077		89.24

		3076		89.22

		3075		89.2

		3074		89.18

		3073		89.15

		3072		89.13

		3071		89.11

		3070		89.09

		3069		89.06

		3068		89.04

		3067		89.02

		3066		88.99

		3065		88.97

		3064		88.94

		3063		88.92

		3062		88.89

		3061		88.87

		3060		88.84

		3059		88.81

		3058		88.78

		3057		88.75

		3056		88.72

		3055		88.69

		3054		88.66

		3053		88.62

		3052		88.58

		3051		88.55

		3050		88.51

		3049		88.47

		3048		88.42

		3047		88.38

		3046		88.34

		3045		88.29

		3044		88.24

		3043		88.2

		3042		88.15

		3041		88.09

		3040		88.04

		3039		87.99

		3038		87.93

		3037		87.87

		3036		87.81

		3035		87.76

		3034		87.69

		3033		87.63

		3032		87.57

		3031		87.51

		3030		87.45

		3029		87.39

		3028		87.33

		3027		87.27

		3026		87.21

		3025		87.15

		3024		87.09

		3023		87.04

		3022		86.98

		3021		86.92

		3020		86.87

		3019		86.81

		3018		86.75

		3017		86.7

		3016		86.64

		3015		86.59

		3014		86.54

		3013		86.48

		3012		86.43

		3011		86.38

		3010		86.33

		3009		86.28

		3008		86.23

		3007		86.19

		3006		86.14

		3005		86.1

		3004		86.06

		3003		86.02

		3002		85.98

		3001		85.95

		3000		85.91

		2999		85.87

		2998		85.83

		2997		85.78

		2996		85.73

		2995		85.69

		2994		85.64

		2993		85.58

		2992		85.53

		2991		85.47

		2990		85.42

		2989		85.36

		2988		85.31

		2987		85.27

		2986		85.22

		2985		85.17

		2984		85.12

		2983		85.07

		2982		85.01

		2981		84.95

		2980		84.88

		2979		84.79

		2978		84.67

		2977		84.53

		2976		84.35

		2975		84.12

		2974		83.84

		2973		83.5

		2972		83.1

		2971		82.64

		2970		82.14

		2969		81.59

		2968		81.02

		2967		80.43

		2966		79.83

		2965		79.24

		2964		78.67

		2963		78.13

		2962		77.62

		2961		77.17

		2960		76.77

		2959		76.43

		2958		76.15

		2957		75.93

		2956		75.79

		2955		75.73

		2954		75.76

		2953		75.85

		2952		76.02

		2951		76.23

		2950		76.46

		2949		76.69

		2948		76.9

		2947		77.05

		2946		77.15

		2945		77.17

		2944		77.1

		2943		76.94

		2942		76.71

		2941		76.4

		2940		76.03

		2939		75.62

		2938		75.19

		2937		74.74

		2936		74.28

		2935		73.81

		2934		73.32

		2933		72.81

		2932		72.26

		2931		71.64

		2930		70.93

		2929		70.12

		2928		69.18

		2927		68.09

		2926		66.84

		2925		65.43

		2924		63.88

		2923		62.2

		2922		60.45

		2921		58.67

		2920		56.94

		2919		55.33

		2918		53.9

		2917		52.72

		2916		51.85

		2915		51.33

		2914		51.18

		2913		51.4

		2912		51.96

		2911		52.82

		2910		53.93

		2909		55.22

		2908		56.63

		2907		58.09

		2906		59.55

		2905		60.97

		2904		62.3

		2903		63.53

		2902		64.64

		2901		65.65

		2900		66.55

		2899		67.36

		2898		68.1

		2897		68.77

		2896		69.4

		2895		69.99

		2894		70.54

		2893		71.08

		2892		71.61

		2891		72.12

		2890		72.63

		2889		73.13

		2888		73.63

		2887		74.11

		2886		74.58

		2885		75.03

		2884		75.44

		2883		75.8

		2882		76.12

		2881		76.36

		2880		76.55

		2879		76.67

		2878		76.73

		2877		76.74

		2876		76.71

		2875		76.65

		2874		76.59

		2873		76.53

		2872		76.5

		2871		76.49

		2870		76.51

		2869		76.55

		2868		76.59

		2867		76.62

		2866		76.61

		2865		76.54

		2864		76.39

		2863		76.12

		2862		75.7

		2861		75.1

		2860		74.31

		2859		73.29

		2858		72.07

		2857		70.64

		2856		69.06

		2855		67.38

		2854		65.65

		2853		63.97

		2852		62.4

		2851		61.06

		2850		60.01

		2849		59.35

		2848		59.11

		2847		59.32

		2846		59.96

		2845		60.98

		2844		62.33

		2843		63.91

		2842		65.66

		2841		67.47

		2840		69.29

		2839		71.03

		2838		72.65

		2837		74.11

		2836		75.39

		2835		76.51

		2834		77.48

		2833		78.31

		2832		79.02

		2831		79.63

		2830		80.17

		2829		80.64

		2828		81.05

		2827		81.42

		2826		81.75

		2825		82.05

		2824		82.32

		2823		82.57

		2822		82.8

		2821		83.01

		2820		83.21

		2819		83.39

		2818		83.56

		2817		83.72

		2816		83.87

		2815		84.01

		2814		84.14

		2813		84.26

		2812		84.38

		2811		84.49

		2810		84.59

		2809		84.69

		2808		84.79

		2807		84.89

		2806		84.98

		2805		85.06

		2804		85.15

		2803		85.23

		2802		85.31

		2801		85.39

		2800		85.47

		2799		85.54

		2798		85.61

		2797		85.68

		2796		85.74

		2795		85.8

		2794		85.86

		2793		85.91

		2792		85.96

		2791		86.01

		2790		86.06

		2789		86.1

		2788		86.14

		2787		86.18

		2786		86.22

		2785		86.26

		2784		86.29

		2783		86.33

		2782		86.36

		2781		86.39

		2780		86.42

		2779		86.44

		2778		86.47

		2777		86.49

		2776		86.52

		2775		86.54

		2774		86.57

		2773		86.59

		2772		86.61

		2771		86.63

		2770		86.66

		2769		86.68

		2768		86.7

		2767		86.73

		2766		86.75

		2765		86.77

		2764		86.8

		2763		86.82

		2762		86.85

		2761		86.87

		2760		86.89

		2759		86.91

		2758		86.94

		2757		86.96

		2756		86.98

		2755		87

		2754		87.02

		2753		87.05

		2752		87.07

		2751		87.09

		2750		87.12

		2749		87.14

		2748		87.16

		2747		87.19

		2746		87.21

		2745		87.24

		2744		87.26

		2743		87.29

		2742		87.31

		2741		87.33

		2740		87.35

		2739		87.37

		2738		87.38

		2737		87.4

		2736		87.41

		2735		87.42

		2734		87.43

		2733		87.45

		2732		87.46

		2731		87.47

		2730		87.48

		2729		87.49

		2728		87.51

		2727		87.52

		2726		87.53

		2725		87.54

		2724		87.55

		2723		87.56

		2722		87.56

		2721		87.56

		2720		87.56

		2719		87.55

		2718		87.54

		2717		87.52

		2716		87.5

		2715		87.48

		2714		87.46

		2713		87.43

		2712		87.4

		2711		87.37

		2710		87.34

		2709		87.31

		2708		87.28

		2707		87.26

		2706		87.23

		2705		87.21

		2704		87.19

		2703		87.17

		2702		87.16

		2701		87.14

		2700		87.12

		2699		87.11

		2698		87.09

		2697		87.07

		2696		87.05

		2695		87.03

		2694		87.01

		2693		86.99

		2692		86.97

		2691		86.95

		2690		86.92

		2689		86.9

		2688		86.88

		2687		86.86

		2686		86.84

		2685		86.82

		2684		86.81

		2683		86.8

		2682		86.79

		2681		86.78

		2680		86.78

		2679		86.77

		2678		86.77

		2677		86.77

		2676		86.77

		2675		86.77

		2674		86.77

		2673		86.77

		2672		86.78

		2671		86.78

		2670		86.78

		2669		86.78

		2668		86.79

		2667		86.79

		2666		86.79

		2665		86.79

		2664		86.79

		2663		86.79

		2662		86.79

		2661		86.79

		2660		86.79

		2659		86.79

		2658		86.79

		2657		86.79

		2656		86.79

		2655		86.79

		2654		86.79

		2653		86.79

		2652		86.79

		2651		86.8

		2650		86.8

		2649		86.81

		2648		86.82

		2647		86.83

		2646		86.84

		2645		86.85

		2644		86.87

		2643		86.88

		2642		86.89

		2641		86.91

		2640		86.92

		2639		86.93

		2638		86.94

		2637		86.95

		2636		86.96

		2635		86.96

		2634		86.97

		2633		86.98

		2632		86.98

		2631		87

		2630		87.01

		2629		87.02

		2628		87.04

		2627		87.06

		2626		87.09

		2625		87.11

		2624		87.14

		2623		87.17

		2622		87.2

		2621		87.23

		2620		87.25

		2619		87.28

		2618		87.3

		2617		87.33

		2616		87.35

		2615		87.37

		2614		87.38

		2613		87.4

		2612		87.41

		2611		87.42

		2610		87.44

		2609		87.45

		2608		87.47

		2607		87.49

		2606		87.5

		2605		87.53

		2604		87.55

		2603		87.57

		2602		87.6

		2601		87.62

		2600		87.65

		2599		87.68

		2598		87.71

		2597		87.74

		2596		87.78

		2595		87.81

		2594		87.84

		2593		87.87

		2592		87.9

		2591		87.93

		2590		87.95

		2589		87.98

		2588		88

		2587		88.02

		2586		88.04

		2585		88.05

		2584		88.07

		2583		88.08

		2582		88.09

		2581		88.11

		2580		88.12

		2579		88.13

		2578		88.14

		2577		88.15

		2576		88.15

		2575		88.16

		2574		88.17

		2573		88.17

		2572		88.18

		2571		88.18

		2570		88.18

		2569		88.19

		2568		88.19

		2567		88.19

		2566		88.19

		2565		88.19

		2564		88.19

		2563		88.19

		2562		88.2

		2561		88.21

		2560		88.21

		2559		88.23

		2558		88.24

		2557		88.26

		2556		88.28

		2555		88.31

		2554		88.34

		2553		88.37

		2552		88.4

		2551		88.44

		2550		88.48

		2549		88.51

		2548		88.55

		2547		88.59

		2546		88.62

		2545		88.66

		2544		88.69

		2543		88.71

		2542		88.74

		2541		88.76

		2540		88.78

		2539		88.79

		2538		88.8

		2537		88.82

		2536		88.83

		2535		88.84

		2534		88.86

		2533		88.88

		2532		88.9

		2531		88.93

		2530		88.96

		2529		89

		2528		89.05

		2527		89.1

		2526		89.15

		2525		89.2

		2524		89.26

		2523		89.31

		2522		89.37

		2521		89.42

		2520		89.46

		2519		89.51

		2518		89.55

		2517		89.58

		2516		89.61

		2515		89.64

		2514		89.67

		2513		89.7

		2512		89.72

		2511		89.75

		2510		89.78

		2509		89.81

		2508		89.85

		2507		89.89

		2506		89.92

		2505		89.96

		2504		90

		2503		90.04

		2502		90.08

		2501		90.12

		2500		90.15

		2499		90.19

		2498		90.21

		2497		90.24

		2496		90.26

		2495		90.27

		2494		90.29

		2493		90.3

		2492		90.32

		2491		90.33

		2490		90.35

		2489		90.36

		2488		90.38

		2487		90.41

		2486		90.43

		2485		90.46

		2484		90.49

		2483		90.53

		2482		90.56

		2481		90.59

		2480		90.62

		2479		90.66

		2478		90.69

		2477		90.71

		2476		90.74

		2475		90.76

		2474		90.78

		2473		90.8

		2472		90.82

		2471		90.83

		2470		90.84

		2469		90.86

		2468		90.87

		2467		90.88

		2466		90.89

		2465		90.91

		2464		90.92

		2463		90.94

		2462		90.96

		2461		90.98

		2460		91

		2459		91.02

		2458		91.05

		2457		91.07

		2456		91.09

		2455		91.12

		2454		91.14

		2453		91.16

		2452		91.18

		2451		91.19

		2450		91.21

		2449		91.22

		2448		91.24

		2447		91.25

		2446		91.26

		2445		91.28

		2444		91.29

		2443		91.3

		2442		91.32

		2441		91.33

		2440		91.35

		2439		91.37

		2438		91.39

		2437		91.41

		2436		91.43

		2435		91.46

		2434		91.48

		2433		91.5

		2432		91.52

		2431		91.54

		2430		91.56

		2429		91.57

		2428		91.59

		2427		91.6

		2426		91.61

		2425		91.62

		2424		91.63

		2423		91.64

		2422		91.64

		2421		91.65

		2420		91.66

		2419		91.67

		2418		91.68

		2417		91.68

		2416		91.7

		2415		91.71

		2414		91.72

		2413		91.73

		2412		91.75

		2411		91.76

		2410		91.78

		2409		91.79

		2408		91.81

		2407		91.82

		2406		91.84

		2405		91.85

		2404		91.86

		2403		91.87

		2402		91.88

		2401		91.89

		2400		91.89

		2399		91.9

		2398		91.91

		2397		91.92

		2396		91.93

		2395		91.94

		2394		91.95

		2393		91.96

		2392		91.97

		2391		91.98

		2390		91.99

		2389		92

		2388		92.02

		2387		92.03

		2386		92.04

		2385		92.05

		2384		92.07

		2383		92.08

		2382		92.09

		2381		92.09

		2380		92.1

		2379		92.11

		2378		92.11

		2377		92.11

		2376		92.11

		2375		92.11

		2374		92.11

		2373		92.11

		2372		92.11

		2371		92.12

		2370		92.12

		2369		92.12

		2368		92.12

		2367		92.12

		2366		92.13

		2365		92.13

		2364		92.13

		2363		92.13

		2362		92.13

		2361		92.13

		2360		92.14

		2359		92.14

		2358		92.15

		2357		92.15

		2356		92.16

		2355		92.16

		2354		92.16

		2353		92.17

		2352		92.17

		2351		92.17

		2350		92.17

		2349		92.16

		2348		92.16

		2347		92.15

		2346		92.15

		2345		92.15

		2344		92.15

		2343		92.15

		2342		92.15

		2341		92.15

		2340		92.15

		2339		92.16

		2338		92.16

		2337		92.16

		2336		92.16

		2335		92.16

		2334		92.16

		2333		92.15

		2332		92.15

		2331		92.14

		2330		92.13

		2329		92.12

		2328		92.11

		2327		92.1

		2326		92.09

		2325		92.09

		2324		92.09

		2323		92.09

		2322		92.1

		2321		92.11

		2320		92.13

		2319		92.15

		2318		92.17

		2317		92.19

		2316		92.21

		2315		92.24

		2314		92.26

		2313		92.29

		2312		92.31

		2311		92.33

		2310		92.35

		2309		92.37

		2308		92.39

		2307		92.41

		2306		92.42

		2305		92.43

		2304		92.44

		2303		92.44

		2302		92.45

		2301		92.45

		2300		92.45

		2299		92.45

		2298		92.45

		2297		92.44

		2296		92.44

		2295		92.43

		2294		92.43

		2293		92.42

		2292		92.42

		2291		92.41

		2290		92.41

		2289		92.41

		2288		92.41

		2287		92.41

		2286		92.41

		2285		92.41

		2284		92.42

		2283		92.42

		2282		92.43

		2281		92.44

		2280		92.45

		2279		92.47

		2278		92.48

		2277		92.49

		2276		92.51

		2275		92.52

		2274		92.54

		2273		92.56

		2272		92.57

		2271		92.59

		2270		92.6

		2269		92.61

		2268		92.62

		2267		92.63

		2266		92.64

		2265		92.65

		2264		92.65

		2263		92.65

		2262		92.66

		2261		92.66

		2260		92.67

		2259		92.68

		2258		92.69

		2257		92.7

		2256		92.72

		2255		92.73

		2254		92.75

		2253		92.77

		2252		92.78

		2251		92.8

		2250		92.82

		2249		92.83

		2248		92.84

		2247		92.85

		2246		92.86

		2245		92.87

		2244		92.87

		2243		92.88

		2242		92.89

		2241		92.89

		2240		92.9

		2239		92.91

		2238		92.92

		2237		92.93

		2236		92.94

		2235		92.95

		2234		92.96

		2233		92.98

		2232		92.99

		2231		93.01

		2230		93.02

		2229		93.03

		2228		93.05

		2227		93.06

		2226		93.07

		2225		93.08

		2224		93.09

		2223		93.09

		2222		93.1

		2221		93.11

		2220		93.11

		2219		93.11

		2218		93.11

		2217		93.11

		2216		93.11

		2215		93.1

		2214		93.1

		2213		93.1

		2212		93.1

		2211		93.1

		2210		93.11

		2209		93.11

		2208		93.12

		2207		93.13

		2206		93.14

		2205		93.14

		2204		93.15

		2203		93.15

		2202		93.15

		2201		93.15

		2200		93.14

		2199		93.13

		2198		93.12

		2197		93.11

		2196		93.1

		2195		93.09

		2194		93.09

		2193		93.09

		2192		93.09

		2191		93.09

		2190		93.1

		2189		93.11

		2188		93.12

		2187		93.14

		2186		93.15

		2185		93.17

		2184		93.19

		2183		93.21

		2182		93.22

		2181		93.23

		2180		93.24

		2179		93.25

		2178		93.26

		2177		93.26

		2176		93.26

		2175		93.25

		2174		93.24

		2173		93.23

		2172		93.22

		2171		93.21

		2170		93.19

		2169		93.18

		2168		93.18

		2167		93.19

		2166		93.21

		2165		93.24

		2164		93.28

		2163		93.32

		2162		93.37

		2161		93.43

		2160		93.49

		2159		93.54

		2158		93.59

		2157		93.62

		2156		93.64

		2155		93.65

		2154		93.66

		2153		93.65

		2152		93.64

		2151		93.63

		2150		93.61

		2149		93.59

		2148		93.58

		2147		93.57

		2146		93.56

		2145		93.56

		2144		93.55

		2143		93.55

		2142		93.55

		2141		93.55

		2140		93.55

		2139		93.56

		2138		93.56

		2137		93.56

		2136		93.56

		2135		93.56

		2134		93.56

		2133		93.55

		2132		93.54

		2131		93.54

		2130		93.53

		2129		93.52

		2128		93.5

		2127		93.49

		2126		93.48

		2125		93.46

		2124		93.45

		2123		93.43

		2122		93.42

		2121		93.4

		2120		93.39

		2119		93.37

		2118		93.36

		2117		93.35

		2116		93.33

		2115		93.32

		2114		93.32

		2113		93.31

		2112		93.31

		2111		93.3

		2110		93.3

		2109		93.3

		2108		93.29

		2107		93.29

		2106		93.29

		2105		93.29

		2104		93.29

		2103		93.29

		2102		93.3

		2101		93.3

		2100		93.31

		2099		93.31

		2098		93.32

		2097		93.33

		2096		93.34

		2095		93.35

		2094		93.35

		2093		93.36

		2092		93.36

		2091		93.36

		2090		93.35

		2089		93.35

		2088		93.34

		2087		93.34

		2086		93.33

		2085		93.32

		2084		93.32

		2083		93.32

		2082		93.31

		2081		93.32

		2080		93.32

		2079		93.32

		2078		93.33

		2077		93.34

		2076		93.34

		2075		93.35

		2074		93.36

		2073		93.37

		2072		93.38

		2071		93.39

		2070		93.39

		2069		93.4

		2068		93.4

		2067		93.41

		2066		93.41

		2065		93.42

		2064		93.42

		2063		93.42

		2062		93.42

		2061		93.42

		2060		93.42

		2059		93.41

		2058		93.41

		2057		93.4

		2056		93.39

		2055		93.39

		2054		93.38

		2053		93.38

		2052		93.37

		2051		93.38

		2050		93.39

		2049		93.4

		2048		93.41

		2047		93.42

		2046		93.43

		2045		93.44

		2044		93.45

		2043		93.46

		2042		93.47

		2041		93.48

		2040		93.48

		2039		93.49

		2038		93.5

		2037		93.51

		2036		93.52

		2035		93.53

		2034		93.54

		2033		93.56

		2032		93.57

		2031		93.58

		2030		93.59

		2029		93.6

		2028		93.61

		2027		93.61

		2026		93.62

		2025		93.62

		2024		93.63

		2023		93.63

		2022		93.63

		2021		93.64

		2020		93.64

		2019		93.64

		2018		93.64

		2017		93.64

		2016		93.65

		2015		93.66

		2014		93.67

		2013		93.68

		2012		93.69

		2011		93.7

		2010		93.71

		2009		93.72

		2008		93.73

		2007		93.73

		2006		93.73

		2005		93.73

		2004		93.71

		2003		93.7

		2002		93.69

		2001		93.67

		2000		93.65

		1999		93.63

		1998		93.61

		1997		93.59

		1996		93.57

		1995		93.56

		1994		93.55

		1993		93.53

		1992		93.52

		1991		93.51

		1990		93.5

		1989		93.48

		1988		93.47

		1987		93.46

		1986		93.46

		1985		93.45

		1984		93.45

		1983		93.45

		1982		93.46

		1981		93.48

		1980		93.5

		1979		93.52

		1978		93.56

		1977		93.59

		1976		93.62

		1975		93.65

		1974		93.68

		1973		93.7

		1972		93.72

		1971		93.73

		1970		93.74

		1969		93.74

		1968		93.74

		1967		93.74

		1966		93.74

		1965		93.74

		1964		93.74

		1963		93.74

		1962		93.75

		1961		93.75

		1960		93.74

		1959		93.74

		1958		93.74

		1957		93.73

		1956		93.72

		1955		93.7

		1954		93.69

		1953		93.68

		1952		93.67

		1951		93.66

		1950		93.65

		1949		93.64

		1948		93.64

		1947		93.63

		1946		93.63

		1945		93.63

		1944		93.63

		1943		93.63

		1942		93.63

		1941		93.63

		1940		93.63

		1939		93.63

		1938		93.63

		1937		93.63

		1936		93.62

		1935		93.61

		1934		93.61

		1933		93.6

		1932		93.59

		1931		93.58

		1930		93.57

		1929		93.56

		1928		93.55

		1927		93.53

		1926		93.52

		1925		93.51

		1924		93.5

		1923		93.49

		1922		93.48

		1921		93.47

		1920		93.46

		1919		93.45

		1918		93.44

		1917		93.44

		1916		93.43

		1915		93.43

		1914		93.42

		1913		93.42

		1912		93.42

		1911		93.42

		1910		93.42

		1909		93.42

		1908		93.41

		1907		93.41

		1906		93.4

		1905		93.39

		1904		93.38

		1903		93.37

		1902		93.36

		1901		93.35

		1900		93.34

		1899		93.33

		1898		93.32

		1897		93.32

		1896		93.32

		1895		93.32

		1894		93.33

		1893		93.33

		1892		93.34

		1891		93.35

		1890		93.35

		1889		93.35

		1888		93.35

		1887		93.35

		1886		93.35

		1885		93.34

		1884		93.34

		1883		93.33

		1882		93.32

		1881		93.31

		1880		93.3

		1879		93.28

		1878		93.27

		1877		93.26

		1876		93.25

		1875		93.24

		1874		93.23

		1873		93.22

		1872		93.21

		1871		93.2

		1870		93.2

		1869		93.19

		1868		93.18

		1867		93.18

		1866		93.17

		1865		93.17

		1864		93.16

		1863		93.15

		1862		93.14

		1861		93.13

		1860		93.12

		1859		93.11

		1858		93.1

		1857		93.09

		1856		93.07

		1855		93.06

		1854		93.05

		1853		93.04

		1852		93.03

		1851		93.02

		1850		93.01

		1849		93

		1848		92.99

		1847		92.98

		1846		92.98

		1845		92.97

		1844		92.96

		1843		92.95

		1842		92.94

		1841		92.93

		1840		92.92

		1839		92.91

		1838		92.9

		1837		92.9

		1836		92.89

		1835		92.88

		1834		92.87

		1833		92.86

		1832		92.85

		1831		92.84

		1830		92.83

		1829		92.81

		1828		92.79

		1827		92.78

		1826		92.76

		1825		92.73

		1824		92.71

		1823		92.69

		1822		92.67

		1821		92.64

		1820		92.62

		1819		92.6

		1818		92.59

		1817		92.57

		1816		92.55

		1815		92.54

		1814		92.53

		1813		92.52

		1812		92.51

		1811		92.5

		1810		92.49

		1809		92.49

		1808		92.48

		1807		92.47

		1806		92.46

		1805		92.45

		1804		92.44

		1803		92.43

		1802		92.41

		1801		92.4

		1800		92.37

		1799		92.35

		1798		92.32

		1797		92.29

		1796		92.25

		1795		92.21

		1794		92.17

		1793		92.13

		1792		92.08

		1791		92.04

		1790		92

		1789		91.96

		1788		91.93

		1787		91.91

		1786		91.89

		1785		91.89

		1784		91.89

		1783		91.9

		1782		91.92

		1781		91.95

		1780		91.99

		1779		92.02

		1778		92.07

		1777		92.11

		1776		92.15

		1775		92.19

		1774		92.23

		1773		92.27

		1772		92.31

		1771		92.34

		1770		92.37

		1769		92.4

		1768		92.43

		1767		92.45

		1766		92.48

		1765		92.5

		1764		92.52

		1763		92.54

		1762		92.56

		1761		92.58

		1760		92.59

		1759		92.61

		1758		92.62

		1757		92.63

		1756		92.63

		1755		92.63

		1754		92.63

		1753		92.63

		1752		92.61

		1751		92.6

		1750		92.58

		1749		92.56

		1748		92.53

		1747		92.5

		1746		92.46

		1745		92.41

		1744		92.36

		1743		92.29

		1742		92.22

		1741		92.13

		1740		92.03

		1739		91.92

		1738		91.79

		1737		91.65

		1736		91.49

		1735		91.3

		1734		91.09

		1733		90.86

		1732		90.6

		1731		90.31

		1730		89.98

		1729		89.61

		1728		89.19

		1727		88.72

		1726		88.16

		1725		87.53

		1724		86.81

		1723		85.99

		1722		85.08

		1721		84.07

		1720		82.96

		1719		81.74

		1718		80.43

		1717		79.02

		1716		77.55

		1715		76

		1714		74.38

		1713		72.71

		1712		70.98

		1711		69.21

		1710		67.4

		1709		65.56

		1708		63.72

		1707		61.88

		1706		60.08

		1705		58.35

		1704		56.73

		1703		55.23

		1702		53.88

		1701		52.7

		1700		51.7

		1699		50.9

		1698		50.3

		1697		49.9

		1696		49.67

		1695		49.58

		1694		49.63

		1693		49.78

		1692		50.05

		1691		50.42

		1690		50.9

		1689		51.47

		1688		52.15

		1687		52.95

		1686		53.88

		1685		54.96

		1684		56.19

		1683		57.58

		1682		59.09

		1681		60.73

		1680		62.46

		1679		64.27

		1678		66.11

		1677		67.96

		1676		69.8

		1675		71.57

		1674		73.26

		1673		74.84

		1672		76.31

		1671		77.66

		1670		78.9

		1669		80.01

		1668		81

		1667		81.89

		1666		82.67

		1665		83.36

		1664		83.98

		1663		84.54

		1662		85.04

		1661		85.49

		1660		85.9

		1659		86.26

		1658		86.59

		1657		86.9

		1656		87.18

		1655		87.43

		1654		87.67

		1653		87.88

		1652		88.08

		1651		88.27

		1650		88.44

		1649		88.6

		1648		88.76

		1647		88.91

		1646		89.05

		1645		89.18

		1644		89.31

		1643		89.44

		1642		89.57

		1641		89.69

		1640		89.81

		1639		89.93

		1638		90.04

		1637		90.14

		1636		90.25

		1635		90.35

		1634		90.45

		1633		90.54

		1632		90.63

		1631		90.72

		1630		90.81

		1629		90.89

		1628		90.97

		1627		91.05

		1626		91.13

		1625		91.21

		1624		91.28

		1623		91.36

		1622		91.43

		1621		91.5

		1620		91.57

		1619		91.64

		1618		91.7

		1617		91.77

		1616		91.83

		1615		91.89

		1614		91.95

		1613		92.01

		1612		92.07

		1611		92.12

		1610		92.17

		1609		92.22

		1608		92.27

		1607		92.31

		1606		92.35

		1605		92.39

		1604		92.43

		1603		92.46

		1602		92.49

		1601		92.51

		1600		92.54

		1599		92.56

		1598		92.58

		1597		92.6

		1596		92.62

		1595		92.64

		1594		92.66

		1593		92.69

		1592		92.71

		1591		92.73

		1590		92.75

		1589		92.76

		1588		92.78

		1587		92.8

		1586		92.82

		1585		92.84

		1584		92.85

		1583		92.87

		1582		92.88

		1581		92.89

		1580		92.9

		1579		92.91

		1578		92.92

		1577		92.92

		1576		92.93

		1575		92.93

		1574		92.93

		1573		92.93

		1572		92.94

		1571		92.94

		1570		92.95

		1569		92.95

		1568		92.96

		1567		92.97

		1566		92.97

		1565		92.99

		1564		93

		1563		93.01

		1562		93.02

		1561		93.03

		1560		93.04

		1559		93.04

		1558		93.05

		1557		93.06

		1556		93.06

		1555		93.06

		1554		93.07

		1553		93.07

		1552		93.08

		1551		93.08

		1550		93.09

		1549		93.09

		1548		93.1

		1547		93.11

		1546		93.12

		1545		93.12

		1544		93.13

		1543		93.14

		1542		93.14

		1541		93.15

		1540		93.16

		1539		93.16

		1538		93.17

		1537		93.17

		1536		93.18

		1535		93.18

		1534		93.19

		1533		93.19

		1532		93.19

		1531		93.19

		1530		93.18

		1529		93.18

		1528		93.17

		1527		93.17

		1526		93.16

		1525		93.15

		1524		93.15

		1523		93.14

		1522		93.13

		1521		93.13

		1520		93.12

		1519		93.11

		1518		93.1

		1517		93.1

		1516		93.09

		1515		93.09

		1514		93.08

		1513		93.07

		1512		93.07

		1511		93.07

		1510		93.06

		1509		93.06

		1508		93.06

		1507		93.05

		1506		93.05

		1505		93.04

		1504		93.03

		1503		93.03

		1502		93.02

		1501		93.01

		1500		92.99

		1499		92.98

		1498		92.96

		1497		92.94

		1496		92.92

		1495		92.9

		1494		92.88

		1493		92.86

		1492		92.83

		1491		92.8

		1490		92.76

		1489		92.71

		1488		92.65

		1487		92.58

		1486		92.47

		1485		92.32

		1484		92.11

		1483		91.79

		1482		91.33

		1481		90.7

		1480		89.91

		1479		88.96

		1478		87.9

		1477		86.74

		1476		85.52

		1475		84.27

		1474		83.03

		1473		81.86

		1472		80.85

		1471		80.08

		1470		79.56

		1469		79.25

		1468		79.12

		1467		79.14

		1466		79.27

		1465		79.52

		1464		79.87

		1463		80.3

		1462		80.78

		1461		81.24

		1460		81.68

		1459		82.09

		1458		82.5

		1457		82.9

		1456		83.29

		1455		83.67

		1454		84

		1453		84.28

		1452		84.5

		1451		84.66

		1450		84.75

		1449		84.79

		1448		84.76

		1447		84.68

		1446		84.55

		1445		84.37

		1444		84.13

		1443		83.85

		1442		83.52

		1441		83.14

		1440		82.71

		1439		82.24

		1438		81.73

		1437		81.2

		1436		80.67

		1435		80.14

		1434		79.66

		1433		79.24

		1432		78.89

		1431		78.65

		1430		78.53

		1429		78.54

		1428		78.67

		1427		78.92

		1426		79.27

		1425		79.68

		1424		80.13

		1423		80.58

		1422		80.99

		1421		81.32

		1420		81.56

		1419		81.68

		1418		81.68

		1417		81.57

		1416		81.37

		1415		81.1

		1414		80.81

		1413		80.54

		1412		80.33

		1411		80.23

		1410		80.25

		1409		80.43

		1408		80.75

		1407		81.21

		1406		81.8

		1405		82.49

		1404		83.25

		1403		84.05

		1402		84.85

		1401		85.62

		1400		86.34

		1399		86.99

		1398		87.57

		1397		88.08

		1396		88.52

		1395		88.88

		1394		89.19

		1393		89.45

		1392		89.66

		1391		89.84

		1390		89.98

		1389		90.09

		1388		90.16

		1387		90.22

		1386		90.24

		1385		90.24

		1384		90.22

		1383		90.18

		1382		90.11

		1381		90.03

		1380		89.93

		1379		89.83

		1378		89.73

		1377		89.63

		1376		89.53

		1375		89.45

		1374		89.37

		1373		89.31

		1372		89.26

		1371		89.22

		1370		89.18

		1369		89.12

		1368		89.06

		1367		88.97

		1366		88.86

		1365		88.73

		1364		88.57

		1363		88.39

		1362		88.19

		1361		87.98

		1360		87.76

		1359		87.53

		1358		87.32

		1357		87.12

		1356		86.94

		1355		86.79

		1354		86.67

		1353		86.59

		1352		86.54

		1351		86.54

		1350		86.59

		1349		86.69

		1348		86.83

		1347		87.02

		1346		87.24

		1345		87.49

		1344		87.74

		1343		87.97

		1342		88.18

		1341		88.34

		1340		88.43

		1339		88.43

		1338		88.35

		1337		88.19

		1336		87.95

		1335		87.66

		1334		87.32

		1333		86.97

		1332		86.63

		1331		86.33

		1330		86.1

		1329		85.94

		1328		85.87

		1327		85.87

		1326		85.93

		1325		86.03

		1324		86.14

		1323		86.22

		1322		86.24

		1321		86.16

		1320		85.95

		1319		85.59

		1318		85.06

		1317		84.38

		1316		83.56

		1315		82.61

		1314		81.59

		1313		80.51

		1312		79.44

		1311		78.42

		1310		77.49

		1309		76.68

		1308		76.03

		1307		75.54

		1306		75.22

		1305		75.03

		1304		74.97

		1303		75

		1302		75.08

		1301		75.19

		1300		75.3

		1299		75.36

		1298		75.35

		1297		75.24

		1296		75.03

		1295		74.72

		1294		74.34

		1293		73.92

		1292		73.48

		1291		73.07

		1290		72.7

		1289		72.43

		1288		72.29

		1287		72.32

		1286		72.56

		1285		73.02

		1284		73.68

		1283		74.52

		1282		75.5

		1281		76.58

		1280		77.72

		1279		78.88

		1278		80

		1277		81.06

		1276		81.99

		1275		82.77

		1274		83.37

		1273		83.77

		1272		83.97

		1271		83.97

		1270		83.8

		1269		83.49

		1268		83.06

		1267		82.55

		1266		82.02

		1265		81.5

		1264		81.06

		1263		80.74

		1262		80.6

		1261		80.65

		1260		80.9

		1259		81.33

		1258		81.91

		1257		82.61

		1256		83.38

		1255		84.18

		1254		84.97

		1253		85.7

		1252		86.34

		1251		86.85

		1250		87.2

		1249		87.38

		1248		87.36

		1247		87.15

		1246		86.75

		1245		86.19

		1244		85.48

		1243		84.66

		1242		83.77

		1241		82.87

		1240		82.02

		1239		81.28

		1238		80.72

		1237		80.39

		1236		80.32

		1235		80.5

		1234		80.9

		1233		81.49

		1232		82.22

		1231		83.04

		1230		83.89

		1229		84.73

		1228		85.48

		1227		86.11

		1226		86.58

		1225		86.87

		1224		86.98

		1223		86.91

		1222		86.67

		1221		86.29

		1220		85.8

		1219		85.21

		1218		84.56

		1217		83.89

		1216		83.25

		1215		82.69

		1214		82.27

		1213		82.02

		1212		81.95

		1211		82.07

		1210		82.37

		1209		82.83

		1208		83.42

		1207		84.11

		1206		84.87

		1205		85.62

		1204		86.33

		1203		86.94

		1202		87.4

		1201		87.68

		1200		87.77

		1199		87.66

		1198		87.37

		1197		86.93

		1196		86.39

		1195		85.78

		1194		85.15

		1193		84.56

		1192		84.07

		1191		83.75

		1190		83.64

		1189		83.74

		1188		84.06

		1187		84.54

		1186		85.16

		1185		85.86

		1184		86.61

		1183		87.38

		1182		88.13

		1181		88.81

		1180		89.41

		1179		89.92

		1178		90.33

		1177		90.66

		1176		90.92

		1175		91.14

		1174		91.33

		1173		91.48

		1172		91.62

		1171		91.74

		1170		91.85

		1169		91.94

		1168		92.03

		1167		92.1

		1166		92.17

		1165		92.24

		1164		92.29

		1163		92.35

		1162		92.4

		1161		92.44

		1160		92.49

		1159		92.52

		1158		92.56

		1157		92.59

		1156		92.63

		1155		92.66

		1154		92.68

		1153		92.71

		1152		92.73

		1151		92.75

		1150		92.77

		1149		92.79

		1148		92.81

		1147		92.82

		1146		92.84

		1145		92.85

		1144		92.86

		1143		92.87

		1142		92.88

		1141		92.88

		1140		92.88

		1139		92.87

		1138		92.86

		1137		92.83

		1136		92.8

		1135		92.74

		1134		92.67

		1133		92.58

		1132		92.48

		1131		92.35

		1130		92.22

		1129		92.09

		1128		91.95

		1127		91.83

		1126		91.72

		1125		91.64

		1124		91.58

		1123		91.55

		1122		91.56

		1121		91.58

		1120		91.63

		1119		91.69

		1118		91.76

		1117		91.82

		1116		91.88

		1115		91.93

		1114		91.97

		1113		91.99

		1112		92

		1111		92.01

		1110		92

		1109		92

		1108		91.99

		1107		91.97

		1106		91.95

		1105		91.9

		1104		91.82

		1103		91.69

		1102		91.5

		1101		91.26

		1100		90.96

		1099		90.61

		1098		90.23

		1097		89.84

		1096		89.45

		1095		89.08

		1094		88.77

		1093		88.55

		1092		88.42

		1091		88.4

		1090		88.47

		1089		88.63

		1088		88.83

		1087		89.08

		1086		89.35

		1085		89.61

		1084		89.86

		1083		90.08

		1082		90.25

		1081		90.38

		1080		90.47

		1079		90.52

		1078		90.55

		1077		90.56

		1076		90.55

		1075		90.54

		1074		90.51

		1073		90.48

		1072		90.44

		1071		90.39

		1070		90.34

		1069		90.29

		1068		90.23

		1067		90.17

		1066		90.12

		1065		90.07

		1064		90.02

		1063		89.98

		1062		89.93

		1061		89.89

		1060		89.85

		1059		89.81

		1058		89.78

		1057		89.75

		1056		89.73

		1055		89.72

		1054		89.71

		1053		89.72

		1052		89.73

		1051		89.76

		1050		89.79

		1049		89.83

		1048		89.87

		1047		89.91

		1046		89.94

		1045		89.96

		1044		89.98

		1043		89.98

		1042		89.98

		1041		89.97

		1040		89.96

		1039		89.95

		1038		89.96

		1037		89.98

		1036		90

		1035		90.04

		1034		90.09

		1033		90.16

		1032		90.25

		1031		90.34

		1030		90.43

		1029		90.51

		1028		90.58

		1027		90.64

		1026		90.69

		1025		90.73

		1024		90.75

		1023		90.76

		1022		90.76

		1021		90.76

		1020		90.74

		1019		90.73

		1018		90.72

		1017		90.7

		1016		90.68

		1015		90.66

		1014		90.64

		1013		90.62

		1012		90.6

		1011		90.57

		1010		90.53

		1009		90.49

		1008		90.44

		1007		90.39

		1006		90.34

		1005		90.29

		1004		90.25

		1003		90.2

		1002		90.17

		1001		90.15

		1000		90.13

		999		90.14

		998		90.15

		997		90.17

		996		90.2

		995		90.22

		994		90.24

		993		90.25

		992		90.24

		991		90.23

		990		90.2

		989		90.15

		988		90.1

		987		90.03

		986		89.97

		985		89.9

		984		89.83

		983		89.76

		982		89.68

		981		89.59

		980		89.48

		979		89.35

		978		89.19

		977		89

		976		88.78

		975		88.53

		974		88.24

		973		87.91

		972		87.56

		971		87.18

		970		86.77

		969		86.35

		968		85.92

		967		85.47

		966		85.02

		965		84.56

		964		84.1

		963		83.64

		962		83.18

		961		82.72

		960		82.26

		959		81.8

		958		81.34

		957		80.87

		956		80.4

		955		79.91

		954		79.42

		953		78.91

		952		78.39

		951		77.85

		950		77.28

		949		76.71

		948		76.12

		947		75.53

		946		74.95

		945		74.39

		944		73.86

		943		73.38

		942		72.96

		941		72.63

		940		72.38

		939		72.23

		938		72.19

		937		72.25

		936		72.42

		935		72.7

		934		73.07

		933		73.52

		932		74.05

		931		74.64

		930		75.27

		929		75.94

		928		76.63

		927		77.32

		926		78.01

		925		78.68

		924		79.32

		923		79.92

		922		80.48

		921		80.98

		920		81.41

		919		81.79

		918		82.09

		917		82.33

		916		82.51

		915		82.63

		914		82.7

		913		82.75

		912		82.78

		911		82.81

		910		82.85

		909		82.91

		908		83.01

		907		83.13

		906		83.3

		905		83.49

		904		83.7

		903		83.91

		902		84.11

		901		84.28

		900		84.41

		899		84.51

		898		84.55

		897		84.55

		896		84.5

		895		84.43

		894		84.34

		893		84.25

		892		84.17

		891		84.12

		890		84.1

		889		84.12

		888		84.2

		887		84.32

		886		84.49

		885		84.7

		884		84.95

		883		85.21

		882		85.47

		881		85.74

		880		86.01

		879		86.27

		878		86.51

		877		86.74

		876		86.95

		875		87.15

		874		87.34

		873		87.51

		872		87.68

		871		87.84

		870		87.99

		869		88.14

		868		88.28

		867		88.42

		866		88.56

		865		88.7

		864		88.83

		863		88.96

		862		89.1

		861		89.23

		860		89.37

		859		89.51

		858		89.66

		857		89.8

		856		89.95

		855		90.09

		854		90.23

		853		90.37

		852		90.5

		851		90.63

		850		90.75

		849		90.87

		848		90.98

		847		91.08

		846		91.17

		845		91.26

		844		91.34

		843		91.42

		842		91.5

		841		91.57

		840		91.64

		839		91.7

		838		91.76

		837		91.82

		836		91.87

		835		91.92

		834		91.97

		833		92.01

		832		92.05

		831		92.08

		830		92.1

		829		92.12

		828		92.12

		827		92.11

		826		92.07

		825		91.99

		824		91.88

		823		91.74

		822		91.57

		821		91.38

		820		91.18

		819		90.99

		818		90.82

		817		90.68

		816		90.59

		815		90.56

		814		90.61

		813		90.73

		812		90.92

		811		91.15

		810		91.41

		809		91.68

		808		91.95

		807		92.21

		806		92.45

		805		92.66

		804		92.84

		803		92.97

		802		93.08

		801		93.16

		800		93.22

		799		93.27

		798		93.31

		797		93.35

		796		93.37

		795		93.39

		794		93.4

		793		93.39

		792		93.37

		791		93.33

		790		93.27

		789		93.2

		788		93.11

		787		93.02

		786		92.92

		785		92.84

		784		92.76

		783		92.7

		782		92.67

		781		92.67

		780		92.7

		779		92.77

		778		92.86

		777		92.96

		776		93.07

		775		93.18

		774		93.28

		773		93.38

		772		93.47

		771		93.53

		770		93.58

		769		93.6

		768		93.61

		767		93.6

		766		93.56

		765		93.5

		764		93.4

		763		93.26

		762		93.07

		761		92.84

		760		92.57

		759		92.29

		758		92

		757		91.72

		756		91.47

		755		91.26

		754		91.12

		753		91.06

		752		91.1

		751		91.22

		750		91.42

		749		91.65

		748		91.9

		747		92.15

		746		92.38

		745		92.57

		744		92.71

		743		92.78

		742		92.77

		741		92.66

		740		92.45

		739		92.12

		738		91.66

		737		91.06

		736		90.32

		735		89.45

		734		88.46

		733		87.37

		732		86.21

		731		84.98

		730		83.72

		729		82.48

		728		81.31

		727		80.29

		726		79.46

		725		78.85

		724		78.47

		723		78.3

		722		78.35

		721		78.63

		720		79.17

		719		79.93

		718		80.89

		717		81.98

		716		83.14

		715		84.3

		714		85.44

		713		86.52

		712		87.52

		711		88.42

		710		89.19

		709		89.82

		708		90.29

		707		90.63

		706		90.86

		705		90.98

		704		91.02

		703		90.99

		702		90.89

		701		90.71

		700		90.46

		699		90.13

		698		89.72

		697		89.25

		696		88.72

		695		88.14

		694		87.53

		693		86.92

		692		86.32

		691		85.77

		690		85.28

		689		84.89

		688		84.59

		687		84.41

		686		84.33

		685		84.36

		684		84.47

		683		84.66

		682		84.91

		681		85.19

		680		85.49

		679		85.8

		678		86.1

		677		86.39

		676		86.65

		675		86.9

		674		87.14

		673		87.36

		672		87.58

		671		87.79

		670		88.01

		669		88.23

		668		88.46

		667		88.7

		666		88.94

		665		89.19

		664		89.44

		663		89.7

		662		89.96

		661		90.22

		660		90.47

		659		90.72

		658		90.95

		657		91.18

		656		91.39

		655		91.58

		654		91.75

		653		91.91

		652		92.04

		651		92.16

		650		92.26

		649		92.34

		648		92.4

		647		92.44

		646		92.47

		645		92.48

		644		92.49

		643		92.48

		642		92.47

		641		92.45

		640		92.44

		639		92.44

		638		92.44

		637		92.45

		636		92.48

		635		92.51

		634		92.56

		633		92.62

		632		92.69

		631		92.76

		630		92.84

		629		92.92

		628		92.99

		627		93.07

		626		93.14

		625		93.2

		624		93.25

		623		93.3

		622		93.34

		621		93.38

		620		93.41

		619		93.44

		618		93.46

		617		93.48

		616		93.5

		615		93.51

		614		93.53

		613		93.55

		612		93.56

		611		93.58

		610		93.6

		609		93.61

		608		93.63

		607		93.65

		606		93.66

		605		93.68

		604		93.69

		603		93.71

		602		93.72

		601		93.73

		600		93.74

		599		93.75

		598		93.75

		597		93.76

		596		93.76

		595		93.76

		594		93.76

		593		93.76

		592		93.76

		591		93.76

		590		93.75

		589		93.75

		588		93.74

		587		93.73

		586		93.72

		585		93.7

		584		93.68

		583		93.66

		582		93.63

		581		93.59

		580		93.55

		579		93.49

		578		93.42

		577		93.34

		576		93.24

		575		93.13

		574		93.01

		573		92.86

		572		92.7

		571		92.52

		570		92.32

		569		92.1

		568		91.87

		567		91.61

		566		91.33

		565		91.03

		564		90.71

		563		90.37

		562		90

		561		89.61

		560		89.19

		559		88.76

		558		88.31

		557		87.85

		556		87.39

		555		86.94

		554		86.5

		553		86.1

		552		85.75

		551		85.46

		550		85.24

		549		85.12

		548		85.09

		547		85.16

		546		85.34

		545		85.62

		544		85.99

		543		86.44

		542		86.95

		541		87.51

		540		88.09

		539		88.68

		538		89.26

		537		89.81

		536		90.32

		535		90.79

		534		91.2

		533		91.56

		532		91.87

		531		92.13

		530		92.36

		529		92.54

		528		92.69

		527		92.82

		526		92.94

		525		93.03

		524		93.12

		523		93.2

		522		93.27

		521		93.34

		520		93.4

		519		93.45

		518		93.5

		517		93.54

		516		93.56

		515		93.57

		514		93.55

		513		93.5

		512		93.41

		511		93.26

		510		93.05

		509		92.78

		508		92.44

		507		92.04

		506		91.6

		505		91.13

		504		90.65

		503		90.19

		502		89.77

		501		89.43

		500		89.19

		499		89.06

		498		89.04

		497		89.15

		496		89.35

		495		89.63

		494		89.97

		493		90.34

		492		90.72

		491		91.09

		490		91.43

		489		91.72

		488		91.97

		487		92.16

		486		92.32

		485		92.44

		484		92.54

		483		92.63

		482		92.71

		481		92.78

		480		92.86

		479		92.93

		478		93

		477		93.08

		476		93.15

		475		93.21

		474		93.27

		473		93.32

		472		93.36

		471		93.4

		470		93.43

		469		93.45

		468		93.48

		467		93.5

		466		93.52

		465		93.54

		464		93.57

		463		93.6

		462		93.62

		461		93.64

		460		93.66

		459		93.66

		458		93.66

		457		93.64

		456		93.61

		455		93.55

		454		93.46

		453		93.36

		452		93.23

		451		93.09

		450		92.91

		449		92.7

		448		92.44

		447		92.13

		446		91.76

		445		91.34

		444		90.88

		443		90.37

		442		89.84

		441		89.31

		440		88.81

		439		88.35

		438		87.99

		437		87.73

		436		87.6

		435		87.62

		434		87.77

		433		88.05

		432		88.44

		431		88.9

		430		89.42

		429		89.96

		428		90.49

		427		90.99

		426		91.44

		425		91.82

		424		92.13

		423		92.37

		422		92.53

		421		92.64

		420		92.69

		419		92.72

		418		92.73

		417		92.73

		416		92.73

		415		92.74

		414		92.76

		413		92.8

		412		92.87

		411		92.96

		410		93.06

		409		93.17

		408		93.29

		407		93.41

		406		93.51

		405		93.61

		404		93.7

		403		93.78

		402		93.85

		401		93.92

		400		93.98
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		Created as New Dataset		Sample 034 By Administrator Date Monday		 June 19 2023

		cm-1		%T

		4000		98.72

		3999		98.72

		3998		98.72

		3997		98.71

		3996		98.71

		3995		98.71

		3994		98.71

		3993		98.71

		3992		98.71

		3991		98.71

		3990		98.71

		3989		98.7

		3988		98.7

		3987		98.7

		3986		98.7

		3985		98.7

		3984		98.7

		3983		98.7

		3982		98.7

		3981		98.7

		3980		98.7

		3979		98.7

		3978		98.7

		3977		98.7

		3976		98.7

		3975		98.7

		3974		98.7

		3973		98.7

		3972		98.7

		3971		98.7

		3970		98.7

		3969		98.71

		3968		98.71

		3967		98.71

		3966		98.71

		3965		98.7

		3964		98.7

		3963		98.7

		3962		98.7

		3961		98.7

		3960		98.7

		3959		98.7

		3958		98.7

		3957		98.7

		3956		98.7

		3955		98.7

		3954		98.69

		3953		98.69

		3952		98.69

		3951		98.69

		3950		98.69

		3949		98.69

		3948		98.69

		3947		98.69

		3946		98.69

		3945		98.69

		3944		98.69

		3943		98.69

		3942		98.69

		3941		98.69

		3940		98.69

		3939		98.69

		3938		98.69

		3937		98.69

		3936		98.69

		3935		98.69

		3934		98.69

		3933		98.69

		3932		98.69

		3931		98.69

		3930		98.69

		3929		98.69

		3928		98.69

		3927		98.69

		3926		98.69

		3925		98.68

		3924		98.68

		3923		98.68

		3922		98.68

		3921		98.68

		3920		98.67

		3919		98.67

		3918		98.67

		3917		98.67

		3916		98.67

		3915		98.67

		3914		98.67

		3913		98.67

		3912		98.67

		3911		98.67

		3910		98.67

		3909		98.67

		3908		98.67

		3907		98.67

		3906		98.68

		3905		98.68

		3904		98.68

		3903		98.68

		3902		98.68

		3901		98.68

		3900		98.68

		3899		98.68

		3898		98.68

		3897		98.68

		3896		98.68

		3895		98.68

		3894		98.68

		3893		98.68

		3892		98.67

		3891		98.67

		3890		98.67

		3889		98.67

		3888		98.67

		3887		98.67

		3886		98.67

		3885		98.67

		3884		98.67

		3883		98.67

		3882		98.67

		3881		98.67

		3880		98.67

		3879		98.67

		3878		98.67

		3877		98.67

		3876		98.67

		3875		98.67

		3874		98.67

		3873		98.67

		3872		98.67

		3871		98.67

		3870		98.67

		3869		98.67

		3868		98.67

		3867		98.67

		3866		98.67

		3865		98.67

		3864		98.67

		3863		98.67

		3862		98.67

		3861		98.67

		3860		98.68

		3859		98.68

		3858		98.68

		3857		98.68

		3856		98.69

		3855		98.69

		3854		98.69

		3853		98.69

		3852		98.69

		3851		98.68

		3850		98.68

		3849		98.68

		3848		98.67

		3847		98.67

		3846		98.66

		3845		98.66

		3844		98.66

		3843		98.65

		3842		98.65

		3841		98.65

		3840		98.65

		3839		98.65

		3838		98.65

		3837		98.65

		3836		98.65

		3835		98.65

		3834		98.65

		3833		98.65

		3832		98.65

		3831		98.65

		3830		98.65

		3829		98.66

		3828		98.66

		3827		98.66

		3826		98.66

		3825		98.66

		3824		98.66

		3823		98.66

		3822		98.66

		3821		98.66

		3820		98.66

		3819		98.66

		3818		98.67

		3817		98.67

		3816		98.67

		3815		98.67

		3814		98.67

		3813		98.67

		3812		98.67

		3811		98.66

		3810		98.66

		3809		98.66

		3808		98.66

		3807		98.66

		3806		98.65

		3805		98.65

		3804		98.65

		3803		98.65

		3802		98.65

		3801		98.64

		3800		98.64

		3799		98.64

		3798		98.64

		3797		98.64

		3796		98.64

		3795		98.64

		3794		98.64

		3793		98.64

		3792		98.64

		3791		98.64

		3790		98.64

		3789		98.64

		3788		98.64

		3787		98.64

		3786		98.64

		3785		98.65

		3784		98.65

		3783		98.65

		3782		98.65

		3781		98.66

		3780		98.66

		3779		98.66

		3778		98.66

		3777		98.66

		3776		98.66

		3775		98.66

		3774		98.67

		3773		98.66

		3772		98.66

		3771		98.66

		3770		98.66

		3769		98.66

		3768		98.66

		3767		98.66

		3766		98.66

		3765		98.65

		3764		98.65

		3763		98.65

		3762		98.65

		3761		98.65

		3760		98.65

		3759		98.65

		3758		98.65

		3757		98.65

		3756		98.65

		3755		98.65

		3754		98.66

		3753		98.66

		3752		98.66

		3751		98.66

		3750		98.66

		3749		98.66

		3748		98.67

		3747		98.67

		3746		98.67

		3745		98.67

		3744		98.67

		3743		98.67

		3742		98.68

		3741		98.68

		3740		98.68

		3739		98.68

		3738		98.69

		3737		98.69

		3736		98.69

		3735		98.7

		3734		98.7

		3733		98.71

		3732		98.71

		3731		98.71

		3730		98.71

		3729		98.71

		3728		98.71

		3727		98.71

		3726		98.7

		3725		98.7

		3724		98.7

		3723		98.7

		3722		98.7

		3721		98.7

		3720		98.69

		3719		98.69

		3718		98.69

		3717		98.69

		3716		98.69

		3715		98.69

		3714		98.69

		3713		98.69

		3712		98.69

		3711		98.69

		3710		98.69

		3709		98.7

		3708		98.7

		3707		98.7

		3706		98.7

		3705		98.7

		3704		98.71

		3703		98.71

		3702		98.71

		3701		98.71

		3700		98.71

		3699		98.71

		3698		98.71

		3697		98.71

		3696		98.72

		3695		98.72

		3694		98.72

		3693		98.72

		3692		98.72

		3691		98.72

		3690		98.71

		3689		98.71

		3688		98.71

		3687		98.71

		3686		98.71

		3685		98.71

		3684		98.71

		3683		98.71

		3682		98.7

		3681		98.7

		3680		98.7

		3679		98.7

		3678		98.7

		3677		98.7

		3676		98.7

		3675		98.7

		3674		98.71

		3673		98.71

		3672		98.71

		3671		98.71

		3670		98.71

		3669		98.71

		3668		98.71

		3667		98.7

		3666		98.7

		3665		98.7

		3664		98.7

		3663		98.7

		3662		98.7

		3661		98.7

		3660		98.7

		3659		98.7

		3658		98.7

		3657		98.7

		3656		98.7

		3655		98.7

		3654		98.7

		3653		98.71

		3652		98.71

		3651		98.71

		3650		98.71

		3649		98.7

		3648		98.7

		3647		98.7

		3646		98.7

		3645		98.7

		3644		98.69

		3643		98.69

		3642		98.69

		3641		98.69

		3640		98.69

		3639		98.69

		3638		98.69

		3637		98.69

		3636		98.69

		3635		98.69

		3634		98.7

		3633		98.7

		3632		98.7

		3631		98.71

		3630		98.71

		3629		98.71

		3628		98.71

		3627		98.71

		3626		98.71

		3625		98.71

		3624		98.71

		3623		98.71

		3622		98.7

		3621		98.7

		3620		98.7

		3619		98.69

		3618		98.69

		3617		98.68

		3616		98.68

		3615		98.67

		3614		98.67

		3613		98.66

		3612		98.66

		3611		98.65

		3610		98.65

		3609		98.64

		3608		98.64

		3607		98.64

		3606		98.64

		3605		98.64

		3604		98.64

		3603		98.64

		3602		98.65

		3601		98.65

		3600		98.66

		3599		98.66

		3598		98.67

		3597		98.67

		3596		98.68

		3595		98.69

		3594		98.69

		3593		98.7

		3592		98.7

		3591		98.7

		3590		98.71

		3589		98.71

		3588		98.71

		3587		98.71

		3586		98.71

		3585		98.71

		3584		98.71

		3583		98.71

		3582		98.71

		3581		98.71

		3580		98.71

		3579		98.71

		3578		98.71

		3577		98.71

		3576		98.71

		3575		98.71

		3574		98.71

		3573		98.71

		3572		98.71

		3571		98.71

		3570		98.71

		3569		98.71

		3568		98.71

		3567		98.71

		3566		98.71

		3565		98.71

		3564		98.71

		3563		98.7

		3562		98.7

		3561		98.7

		3560		98.7

		3559		98.69

		3558		98.69

		3557		98.69

		3556		98.69

		3555		98.69

		3554		98.68

		3553		98.68

		3552		98.68

		3551		98.68

		3550		98.68

		3549		98.68

		3548		98.68

		3547		98.67

		3546		98.67

		3545		98.67

		3544		98.67

		3543		98.67

		3542		98.67

		3541		98.67

		3540		98.67

		3539		98.67

		3538		98.67

		3537		98.67

		3536		98.67

		3535		98.67

		3534		98.67

		3533		98.67

		3532		98.67

		3531		98.67

		3530		98.67

		3529		98.67

		3528		98.67

		3527		98.67

		3526		98.67

		3525		98.67

		3524		98.67

		3523		98.67

		3522		98.67

		3521		98.67

		3520		98.67

		3519		98.67

		3518		98.67

		3517		98.67

		3516		98.67

		3515		98.66

		3514		98.66

		3513		98.66

		3512		98.67

		3511		98.67

		3510		98.67

		3509		98.67

		3508		98.67

		3507		98.67

		3506		98.67

		3505		98.67

		3504		98.67

		3503		98.67

		3502		98.67

		3501		98.67

		3500		98.67

		3499		98.66

		3498		98.66

		3497		98.66

		3496		98.66

		3495		98.66

		3494		98.66

		3493		98.66

		3492		98.66

		3491		98.66

		3490		98.66

		3489		98.66

		3488		98.66

		3487		98.65

		3486		98.65

		3485		98.65

		3484		98.65

		3483		98.65

		3482		98.65

		3481		98.65

		3480		98.64

		3479		98.64

		3478		98.64

		3477		98.64

		3476		98.64

		3475		98.64

		3474		98.64

		3473		98.64

		3472		98.64

		3471		98.64

		3470		98.64

		3469		98.64

		3468		98.63

		3467		98.63

		3466		98.63

		3465		98.63

		3464		98.63

		3463		98.63

		3462		98.63

		3461		98.63

		3460		98.62

		3459		98.62

		3458		98.62

		3457		98.62

		3456		98.61

		3455		98.61

		3454		98.61

		3453		98.61

		3452		98.61

		3451		98.61

		3450		98.6

		3449		98.6

		3448		98.6

		3447		98.6

		3446		98.6

		3445		98.6

		3444		98.6

		3443		98.6

		3442		98.6

		3441		98.6

		3440		98.6

		3439		98.6

		3438		98.6

		3437		98.59

		3436		98.59

		3435		98.59

		3434		98.58

		3433		98.58

		3432		98.57

		3431		98.56

		3430		98.55

		3429		98.54

		3428		98.54

		3427		98.53

		3426		98.52

		3425		98.51

		3424		98.5

		3423		98.49

		3422		98.49

		3421		98.48

		3420		98.48

		3419		98.47

		3418		98.47

		3417		98.47

		3416		98.47

		3415		98.46

		3414		98.46

		3413		98.46

		3412		98.46

		3411		98.46

		3410		98.46

		3409		98.46

		3408		98.46

		3407		98.46

		3406		98.46

		3405		98.46

		3404		98.47

		3403		98.47

		3402		98.47

		3401		98.47

		3400		98.47

		3399		98.47

		3398		98.47

		3397		98.47

		3396		98.46

		3395		98.45

		3394		98.45

		3393		98.44

		3392		98.43

		3391		98.42

		3390		98.41

		3389		98.39

		3388		98.38

		3387		98.38

		3386		98.37

		3385		98.36

		3384		98.36

		3383		98.36

		3382		98.36

		3381		98.36

		3380		98.36

		3379		98.37

		3378		98.37

		3377		98.38

		3376		98.38

		3375		98.39

		3374		98.4

		3373		98.4

		3372		98.41

		3371		98.41

		3370		98.41

		3369		98.41

		3368		98.41

		3367		98.4

		3366		98.4

		3365		98.39

		3364		98.38

		3363		98.37

		3362		98.36

		3361		98.35

		3360		98.35

		3359		98.34

		3358		98.34

		3357		98.33

		3356		98.33

		3355		98.33

		3354		98.33

		3353		98.33

		3352		98.33

		3351		98.32

		3350		98.32

		3349		98.32

		3348		98.32

		3347		98.31

		3346		98.31

		3345		98.3

		3344		98.3

		3343		98.29

		3342		98.28

		3341		98.28

		3340		98.27

		3339		98.27

		3338		98.26

		3337		98.26

		3336		98.25

		3335		98.24

		3334		98.24

		3333		98.23

		3332		98.23

		3331		98.22

		3330		98.22

		3329		98.22

		3328		98.21

		3327		98.21

		3326		98.21

		3325		98.21

		3324		98.2

		3323		98.2

		3322		98.2

		3321		98.2

		3320		98.2

		3319		98.2

		3318		98.19

		3317		98.19

		3316		98.19

		3315		98.19

		3314		98.19

		3313		98.19

		3312		98.19

		3311		98.19

		3310		98.19

		3309		98.19

		3308		98.19

		3307		98.19

		3306		98.19

		3305		98.18

		3304		98.18

		3303		98.18

		3302		98.17

		3301		98.17

		3300		98.16

		3299		98.15

		3298		98.15

		3297		98.14

		3296		98.13

		3295		98.13

		3294		98.12

		3293		98.11

		3292		98.1

		3291		98.09

		3290		98.08

		3289		98.08

		3288		98.07

		3287		98.06

		3286		98.05

		3285		98.04

		3284		98.03

		3283		98.03

		3282		98.02

		3281		98.01

		3280		98.01

		3279		98

		3278		97.99

		3277		97.99

		3276		97.98

		3275		97.98

		3274		97.97

		3273		97.96

		3272		97.95

		3271		97.94

		3270		97.94

		3269		97.93

		3268		97.92

		3267		97.91

		3266		97.89

		3265		97.88

		3264		97.87

		3263		97.86

		3262		97.85

		3261		97.84

		3260		97.83

		3259		97.82

		3258		97.81

		3257		97.8

		3256		97.79

		3255		97.78

		3254		97.77

		3253		97.76

		3252		97.75

		3251		97.74

		3250		97.73

		3249		97.72

		3248		97.71

		3247		97.7

		3246		97.69

		3245		97.67

		3244		97.66

		3243		97.65

		3242		97.64

		3241		97.62

		3240		97.61

		3239		97.6

		3238		97.58

		3237		97.57

		3236		97.56

		3235		97.55

		3234		97.53

		3233		97.52

		3232		97.5

		3231		97.49

		3230		97.48

		3229		97.46

		3228		97.45

		3227		97.43

		3226		97.42

		3225		97.4

		3224		97.39

		3223		97.38

		3222		97.36

		3221		97.35

		3220		97.34

		3219		97.32

		3218		97.31

		3217		97.29

		3216		97.28

		3215		97.27

		3214		97.25

		3213		97.24

		3212		97.22

		3211		97.21

		3210		97.19

		3209		97.18

		3208		97.16

		3207		97.14

		3206		97.13

		3205		97.11

		3204		97.1

		3203		97.08

		3202		97.07

		3201		97.05

		3200		97.04

		3199		97.02

		3198		97.01

		3197		97

		3196		96.98

		3195		96.97

		3194		96.96

		3193		96.95

		3192		96.93

		3191		96.92

		3190		96.91

		3189		96.89

		3188		96.88

		3187		96.86

		3186		96.85

		3185		96.84

		3184		96.82

		3183		96.81

		3182		96.79

		3181		96.78

		3180		96.77

		3179		96.75

		3178		96.74

		3177		96.73

		3176		96.71

		3175		96.7

		3174		96.69

		3173		96.67

		3172		96.66

		3171		96.64

		3170		96.63

		3169		96.61

		3168		96.59

		3167		96.58

		3166		96.56

		3165		96.54

		3164		96.53

		3163		96.51

		3162		96.49

		3161		96.48

		3160		96.46

		3159		96.44

		3158		96.42

		3157		96.41

		3156		96.39

		3155		96.37

		3154		96.35

		3153		96.33

		3152		96.31

		3151		96.29

		3150		96.27

		3149		96.24

		3148		96.22

		3147		96.2

		3146		96.18

		3145		96.15

		3144		96.13

		3143		96.1

		3142		96.08

		3141		96.05

		3140		96.03

		3139		96

		3138		95.98

		3137		95.95

		3136		95.92

		3135		95.9

		3134		95.87

		3133		95.84

		3132		95.81

		3131		95.79

		3130		95.76

		3129		95.73

		3128		95.7

		3127		95.67

		3126		95.64

		3125		95.61

		3124		95.59

		3123		95.56

		3122		95.53

		3121		95.5

		3120		95.47

		3119		95.44

		3118		95.41

		3117		95.38

		3116		95.35

		3115		95.32

		3114		95.29

		3113		95.26

		3112		95.23

		3111		95.2

		3110		95.17

		3109		95.14

		3108		95.11

		3107		95.08

		3106		95.05

		3105		95.02

		3104		94.99

		3103		94.96

		3102		94.94

		3101		94.91

		3100		94.88

		3099		94.86

		3098		94.83

		3097		94.81

		3096		94.78

		3095		94.76

		3094		94.74

		3093		94.72

		3092		94.7

		3091		94.68

		3090		94.66

		3089		94.64

		3088		94.63

		3087		94.61

		3086		94.59

		3085		94.57

		3084		94.56

		3083		94.54

		3082		94.52

		3081		94.5

		3080		94.48

		3079		94.47

		3078		94.45

		3077		94.43

		3076		94.41

		3075		94.39

		3074		94.37

		3073		94.35

		3072		94.33

		3071		94.3

		3070		94.28

		3069		94.26

		3068		94.24

		3067		94.22

		3066		94.2

		3065		94.18

		3064		94.16

		3063		94.13

		3062		94.11

		3061		94.09

		3060		94.06

		3059		94.04

		3058		94.01

		3057		93.98

		3056		93.96

		3055		93.93

		3054		93.9

		3053		93.87

		3052		93.84

		3051		93.8

		3050		93.77

		3049		93.74

		3048		93.7

		3047		93.67

		3046		93.63

		3045		93.6

		3044		93.56

		3043		93.52

		3042		93.49

		3041		93.45

		3040		93.41

		3039		93.37

		3038		93.33

		3037		93.29

		3036		93.25

		3035		93.21

		3034		93.16

		3033		93.12

		3032		93.09

		3031		93.05

		3030		93.01

		3029		92.98

		3028		92.94

		3027		92.91

		3026		92.88

		3025		92.85

		3024		92.82

		3023		92.8

		3022		92.78

		3021		92.75

		3020		92.73

		3019		92.72

		3018		92.7

		3017		92.69

		3016		92.68

		3015		92.67

		3014		92.66

		3013		92.66

		3012		92.66

		3011		92.66

		3010		92.66

		3009		92.67

		3008		92.68

		3007		92.69

		3006		92.7

		3005		92.71

		3004		92.73

		3003		92.74

		3002		92.76

		3001		92.78

		3000		92.79

		2999		92.81

		2998		92.82

		2997		92.83

		2996		92.84

		2995		92.85

		2994		92.86

		2993		92.86

		2992		92.86

		2991		92.86

		2990		92.86

		2989		92.85

		2988		92.84

		2987		92.82

		2986		92.8

		2985		92.78

		2984		92.74

		2983		92.7

		2982		92.66

		2981		92.6

		2980		92.53

		2979		92.45

		2978		92.34

		2977		92.21

		2976		92.04

		2975		91.83

		2974		91.56

		2973		91.24

		2972		90.85

		2971		90.4

		2970		89.91

		2969		89.37

		2968		88.81

		2967		88.22

		2966		87.63

		2965		87.05

		2964		86.49

		2963		85.96

		2962		85.48

		2961		85.06

		2960		84.7

		2959		84.39

		2958		84.15

		2957		83.98

		2956		83.87

		2955		83.84

		2954		83.87

		2953		83.97

		2952		84.12

		2951		84.29

		2950		84.48

		2949		84.66

		2948		84.82

		2947		84.92

		2946		84.97

		2945		84.95

		2944		84.85

		2943		84.67

		2942		84.42

		2941		84.1

		2940		83.74

		2939		83.34

		2938		82.92

		2937		82.5

		2936		82.06

		2935		81.63

		2934		81.19

		2933		80.73

		2932		80.25

		2931		79.72

		2930		79.13

		2929		78.46

		2928		77.69

		2927		76.8

		2926		75.79

		2925		74.66

		2924		73.42

		2923		72.08

		2922		70.69

		2921		69.29

		2920		67.94

		2919		66.7

		2918		65.62

		2917		64.75

		2916		64.14

		2915		63.83

		2914		63.82

		2913		64.11

		2912		64.69

		2911		65.51

		2910		66.53

		2909		67.68

		2908		68.91

		2907		70.18

		2906		71.42

		2905		72.62

		2904		73.74

		2903		74.76

		2902		75.67

		2901		76.49

		2900		77.21

		2899		77.86

		2898		78.44

		2897		78.96

		2896		79.45

		2895		79.9

		2894		80.33

		2893		80.75

		2892		81.15

		2891		81.55

		2890		81.94

		2889		82.33

		2888		82.72

		2887		83.09

		2886		83.45

		2885		83.79

		2884		84.09

		2883		84.35

		2882		84.56

		2881		84.72

		2880		84.82

		2879		84.86

		2878		84.85

		2877		84.8

		2876		84.72

		2875		84.61

		2874		84.51

		2873		84.41

		2872		84.33

		2871		84.29

		2870		84.26

		2869		84.26

		2868		84.26

		2867		84.26

		2866		84.22

		2865		84.13

		2864		83.97

		2863		83.71

		2862		83.33

		2861		82.81

		2860		82.13

		2859		81.27

		2858		80.25

		2857		79.08

		2856		77.8

		2855		76.44

		2854		75.05

		2853		73.71

		2852		72.48

		2851		71.42

		2850		70.62

		2849		70.12

		2848		69.96

		2847		70.16

		2846		70.7

		2845		71.56

		2844		72.67

		2843		73.97

		2842		75.4

		2841		76.88

		2840		78.37

		2839		79.79

		2838		81.12

		2837		82.31

		2836		83.37

		2835		84.29

		2834		85.08

		2833		85.76

		2832		86.34

		2831		86.84

		2830		87.28

		2829		87.66

		2828		88

		2827		88.3

		2826		88.56

		2825		88.8

		2824		89.02

		2823		89.21

		2822		89.4

		2821		89.56

		2820		89.71

		2819		89.85

		2818		89.98

		2817		90.1

		2816		90.21

		2815		90.32

		2814		90.42

		2813		90.51

		2812		90.59

		2811		90.67

		2810		90.75

		2809		90.82

		2808		90.89

		2807		90.96

		2806		91.03

		2805		91.09

		2804		91.15

		2803		91.21

		2802		91.27

		2801		91.33

		2800		91.38

		2799		91.44

		2798		91.49

		2797		91.54

		2796		91.58

		2795		91.63

		2794		91.67

		2793		91.71

		2792		91.74

		2791		91.78

		2790		91.81

		2789		91.84

		2788		91.87

		2787		91.9

		2786		91.92

		2785		91.95

		2784		91.97

		2783		91.99

		2782		92.01

		2781		92.03

		2780		92.05

		2779		92.06

		2778		92.08

		2777		92.1

		2776		92.11

		2775		92.12

		2774		92.14

		2773		92.15

		2772		92.17

		2771		92.18

		2770		92.2

		2769		92.21

		2768		92.23

		2767		92.24

		2766		92.26

		2765		92.27

		2764		92.29

		2763		92.31

		2762		92.32

		2761		92.34

		2760		92.36

		2759		92.38

		2758		92.39

		2757		92.41

		2756		92.43

		2755		92.44

		2754		92.46

		2753		92.48

		2752		92.5

		2751		92.52

		2750		92.53

		2749		92.55

		2748		92.57

		2747		92.59

		2746		92.61

		2745		92.64

		2744		92.66

		2743		92.67

		2742		92.69

		2741		92.71

		2740		92.73

		2739		92.74

		2738		92.76

		2737		92.77

		2736		92.78

		2735		92.79

		2734		92.8

		2733		92.81

		2732		92.82

		2731		92.83

		2730		92.84

		2729		92.85

		2728		92.86

		2727		92.87

		2726		92.88

		2725		92.89

		2724		92.89

		2723		92.9

		2722		92.9

		2721		92.9

		2720		92.89

		2719		92.88

		2718		92.87

		2717		92.85

		2716		92.82

		2715		92.8

		2714		92.77

		2713		92.74

		2712		92.7

		2711		92.67

		2710		92.63

		2709		92.6

		2708		92.57

		2707		92.54

		2706		92.51

		2705		92.48

		2704		92.45

		2703		92.43

		2702		92.41

		2701		92.38

		2700		92.36

		2699		92.34

		2698		92.32

		2697		92.3

		2696		92.28

		2695		92.26

		2694		92.23

		2693		92.21

		2692		92.19

		2691		92.16

		2690		92.14

		2689		92.11

		2688		92.09

		2687		92.07

		2686		92.05

		2685		92.03

		2684		92.01

		2683		91.99

		2682		91.98

		2681		91.97

		2680		91.96

		2679		91.95

		2678		91.94

		2677		91.94

		2676		91.94

		2675		91.94

		2674		91.94

		2673		91.94

		2672		91.94

		2671		91.94

		2670		91.94

		2669		91.94

		2668		91.95

		2667		91.95

		2666		91.95

		2665		91.95

		2664		91.95

		2663		91.95

		2662		91.95

		2661		91.95

		2660		91.94

		2659		91.94

		2658		91.94

		2657		91.93

		2656		91.93

		2655		91.93

		2654		91.92

		2653		91.92

		2652		91.92

		2651		91.92

		2650		91.93

		2649		91.93

		2648		91.94

		2647		91.95

		2646		91.96

		2645		91.97

		2644		91.98

		2643		91.99

		2642		92.01

		2641		92.02

		2640		92.03

		2639		92.03

		2638		92.04

		2637		92.04

		2636		92.05

		2635		92.05

		2634		92.05

		2633		92.05

		2632		92.06

		2631		92.06

		2630		92.07

		2629		92.08

		2628		92.09

		2627		92.1

		2626		92.12

		2625		92.14

		2624		92.17

		2623		92.19

		2622		92.22

		2621		92.25

		2620		92.27

		2619		92.3

		2618		92.32

		2617		92.34

		2616		92.36

		2615		92.37

		2614		92.39

		2613		92.4

		2612		92.41

		2611		92.42

		2610		92.42

		2609		92.43

		2608		92.44

		2607		92.45

		2606		92.47

		2605		92.48

		2604		92.5

		2603		92.52

		2602		92.54

		2601		92.57

		2600		92.59

		2599		92.62

		2598		92.65

		2597		92.68

		2596		92.71

		2595		92.74

		2594		92.77

		2593		92.8

		2592		92.83

		2591		92.85

		2590		92.88

		2589		92.9

		2588		92.92

		2587		92.93

		2586		92.95

		2585		92.96

		2584		92.97

		2583		92.98

		2582		92.99

		2581		93

		2580		93

		2579		93.01

		2578		93.02

		2577		93.02

		2576		93.03

		2575		93.03

		2574		93.03

		2573		93.04

		2572		93.04

		2571		93.04

		2570		93.04

		2569		93.04

		2568		93.04

		2567		93.05

		2566		93.05

		2565		93.05

		2564		93.05

		2563		93.05

		2562		93.05

		2561		93.06

		2560		93.06

		2559		93.07

		2558		93.08

		2557		93.1

		2556		93.12

		2555		93.14

		2554		93.17

		2553		93.2

		2552		93.23

		2551		93.26

		2550		93.3

		2549		93.33

		2548		93.37

		2547		93.4

		2546		93.43

		2545		93.47

		2544		93.49

		2543		93.52

		2542		93.54

		2541		93.56

		2540		93.58

		2539		93.59

		2538		93.6

		2537		93.61

		2536		93.62

		2535		93.64

		2534		93.65

		2533		93.67

		2532		93.69

		2531		93.72

		2530		93.75

		2529		93.79

		2528		93.84

		2527		93.88

		2526		93.94

		2525		93.99

		2524		94.05

		2523		94.1

		2522		94.16

		2521		94.21

		2520		94.26

		2519		94.3

		2518		94.34

		2517		94.38

		2516		94.41

		2515		94.44

		2514		94.47

		2513		94.5

		2512		94.52

		2511		94.55

		2510		94.59

		2509		94.62

		2508		94.65

		2507		94.69

		2506		94.73

		2505		94.77

		2504		94.82

		2503		94.86

		2502		94.9

		2501		94.94

		2500		94.97

		2499		95.01

		2498		95.04

		2497		95.07

		2496		95.09

		2495		95.11

		2494		95.13

		2493		95.15

		2492		95.16

		2491		95.18

		2490		95.2

		2489		95.22

		2488		95.24

		2487		95.26

		2486		95.29

		2485		95.31

		2484		95.34

		2483		95.38

		2482		95.41

		2481		95.45

		2480		95.48

		2479		95.52

		2478		95.55

		2477		95.58

		2476		95.61

		2475		95.64

		2474		95.66

		2473		95.68

		2472		95.7

		2471		95.72

		2470		95.73

		2469		95.74

		2468		95.76

		2467		95.77

		2466		95.78

		2465		95.8

		2464		95.81

		2463		95.83

		2462		95.85

		2461		95.87

		2460		95.89

		2459		95.91

		2458		95.93

		2457		95.95

		2456		95.98

		2455		96

		2454		96.02

		2453		96.04

		2452		96.06

		2451		96.08

		2450		96.1

		2449		96.12

		2448		96.13

		2447		96.15

		2446		96.16

		2445		96.18

		2444		96.19

		2443		96.21

		2442		96.23

		2441		96.24

		2440		96.26

		2439		96.28

		2438		96.3

		2437		96.33

		2436		96.35

		2435		96.37

		2434		96.39

		2433		96.41

		2432		96.44

		2431		96.46

		2430		96.47

		2429		96.49

		2428		96.51

		2427		96.52

		2426		96.54

		2425		96.55

		2424		96.56

		2423		96.57

		2422		96.58

		2421		96.59

		2420		96.61

		2419		96.62

		2418		96.63

		2417		96.64

		2416		96.65

		2415		96.67

		2414		96.68

		2413		96.7

		2412		96.71

		2411		96.73

		2410		96.74

		2409		96.76

		2408		96.77

		2407		96.79

		2406		96.8

		2405		96.81

		2404		96.83

		2403		96.84

		2402		96.85

		2401		96.86

		2400		96.87

		2399		96.87

		2398		96.88

		2397		96.89

		2396		96.9

		2395		96.91

		2394		96.92

		2393		96.93

		2392		96.95

		2391		96.96

		2390		96.98

		2389		96.99

		2388		97.01

		2387		97.03

		2386		97.05

		2385		97.07

		2384		97.09

		2383		97.1

		2382		97.12

		2381		97.13

		2380		97.15

		2379		97.16

		2378		97.17

		2377		97.18

		2376		97.18

		2375		97.19

		2374		97.2

		2373		97.21

		2372		97.21

		2371		97.22

		2370		97.23

		2369		97.24

		2368		97.25

		2367		97.26

		2366		97.27

		2365		97.27

		2364		97.28

		2363		97.28

		2362		97.29

		2361		97.29

		2360		97.29

		2359		97.29

		2358		97.29

		2357		97.29

		2356		97.29

		2355		97.29

		2354		97.29

		2353		97.3

		2352		97.3

		2351		97.3

		2350		97.31

		2349		97.31

		2348		97.31

		2347		97.32

		2346		97.32

		2345		97.32

		2344		97.32

		2343		97.32

		2342		97.32

		2341		97.32

		2340		97.32

		2339		97.32

		2338		97.32

		2337		97.32

		2336		97.31

		2335		97.31

		2334		97.3

		2333		97.29

		2332		97.28

		2331		97.27

		2330		97.26

		2329		97.25

		2328		97.23

		2327		97.22

		2326		97.21

		2325		97.2

		2324		97.2

		2323		97.2

		2322		97.21

		2321		97.22

		2320		97.24

		2319		97.26

		2318		97.28

		2317		97.3

		2316		97.32

		2315		97.34

		2314		97.36

		2313		97.38

		2312		97.4

		2311		97.41

		2310		97.43

		2309		97.44

		2308		97.45

		2307		97.46

		2306		97.47

		2305		97.47

		2304		97.48

		2303		97.48

		2302		97.48

		2301		97.48

		2300		97.48

		2299		97.47

		2298		97.47

		2297		97.46

		2296		97.46

		2295		97.45

		2294		97.45

		2293		97.44

		2292		97.43

		2291		97.43

		2290		97.43

		2289		97.42

		2288		97.42

		2287		97.42

		2286		97.43

		2285		97.43

		2284		97.44

		2283		97.45

		2282		97.45

		2281		97.46

		2280		97.47

		2279		97.48

		2278		97.49

		2277		97.51

		2276		97.52

		2275		97.53

		2274		97.54

		2273		97.55

		2272		97.56

		2271		97.57

		2270		97.59

		2269		97.59

		2268		97.6

		2267		97.61

		2266		97.62

		2265		97.62

		2264		97.63

		2263		97.63

		2262		97.64

		2261		97.65

		2260		97.66

		2259		97.67

		2258		97.68

		2257		97.7

		2256		97.71

		2255		97.73

		2254		97.75

		2253		97.77

		2252		97.79

		2251		97.8

		2250		97.82

		2249		97.83

		2248		97.84

		2247		97.85

		2246		97.86

		2245		97.87

		2244		97.88

		2243		97.88

		2242		97.89

		2241		97.9

		2240		97.91

		2239		97.92

		2238		97.93

		2237		97.94

		2236		97.95

		2235		97.96

		2234		97.97

		2233		97.98

		2232		97.99

		2231		97.99

		2230		98

		2229		98.01

		2228		98.02

		2227		98.03

		2226		98.03

		2225		98.04

		2224		98.05

		2223		98.06

		2222		98.07

		2221		98.07

		2220		98.08

		2219		98.08

		2218		98.08

		2217		98.09

		2216		98.09

		2215		98.09

		2214		98.09

		2213		98.09

		2212		98.09

		2211		98.09

		2210		98.09

		2209		98.1

		2208		98.1

		2207		98.11

		2206		98.11

		2205		98.12

		2204		98.12

		2203		98.12

		2202		98.13

		2201		98.13

		2200		98.13

		2199		98.13

		2198		98.12

		2197		98.12

		2196		98.11

		2195		98.1

		2194		98.1

		2193		98.1

		2192		98.1

		2191		98.1

		2190		98.1

		2189		98.11

		2188		98.12

		2187		98.12

		2186		98.13

		2185		98.14

		2184		98.15

		2183		98.16

		2182		98.17

		2181		98.17

		2180		98.18

		2179		98.18

		2178		98.18

		2177		98.18

		2176		98.18

		2175		98.17

		2174		98.17

		2173		98.16

		2172		98.14

		2171		98.13

		2170		98.12

		2169		98.11

		2168		98.11

		2167		98.11

		2166		98.13

		2165		98.16

		2164		98.19

		2163		98.24

		2162		98.29

		2161		98.35

		2160		98.4

		2159		98.46

		2158		98.51

		2157		98.55

		2156		98.57

		2155		98.59

		2154		98.6

		2153		98.61

		2152		98.6

		2151		98.59

		2150		98.58

		2149		98.56

		2148		98.55

		2147		98.54

		2146		98.53

		2145		98.53

		2144		98.52

		2143		98.52

		2142		98.52

		2141		98.53

		2140		98.53

		2139		98.54

		2138		98.54

		2137		98.55

		2136		98.55

		2135		98.55

		2134		98.55

		2133		98.55

		2132		98.55

		2131		98.54

		2130		98.53

		2129		98.52

		2128		98.51

		2127		98.49

		2126		98.48

		2125		98.47

		2124		98.46

		2123		98.44

		2122		98.43

		2121		98.42

		2120		98.4

		2119		98.39

		2118		98.38

		2117		98.36

		2116		98.35

		2115		98.34

		2114		98.33

		2113		98.33

		2112		98.32

		2111		98.32

		2110		98.32

		2109		98.32

		2108		98.33

		2107		98.33

		2106		98.33

		2105		98.34

		2104		98.34

		2103		98.34

		2102		98.35

		2101		98.35

		2100		98.35

		2099		98.36

		2098		98.36

		2097		98.37

		2096		98.37

		2095		98.38

		2094		98.38

		2093		98.38

		2092		98.38

		2091		98.38

		2090		98.38

		2089		98.38

		2088		98.37

		2087		98.36

		2086		98.36

		2085		98.35

		2084		98.34

		2083		98.34

		2082		98.34

		2081		98.34

		2080		98.34

		2079		98.34

		2078		98.35

		2077		98.36

		2076		98.37

		2075		98.37

		2074		98.38

		2073		98.39

		2072		98.4

		2071		98.41

		2070		98.41

		2069		98.41

		2068		98.42

		2067		98.42

		2066		98.42

		2065		98.41

		2064		98.41

		2063		98.41

		2062		98.41

		2061		98.41

		2060		98.4

		2059		98.4

		2058		98.39

		2057		98.38

		2056		98.37

		2055		98.36

		2054		98.36

		2053		98.35

		2052		98.34

		2051		98.34

		2050		98.34

		2049		98.35

		2048		98.36

		2047		98.37

		2046		98.37

		2045		98.38

		2044		98.39

		2043		98.4

		2042		98.41

		2041		98.42

		2040		98.43

		2039		98.44

		2038		98.46

		2037		98.47

		2036		98.49

		2035		98.51

		2034		98.52

		2033		98.54

		2032		98.55

		2031		98.56

		2030		98.57

		2029		98.57

		2028		98.56

		2027		98.56

		2026		98.55

		2025		98.54

		2024		98.52

		2023		98.51

		2022		98.51

		2021		98.5

		2020		98.5

		2019		98.5

		2018		98.5

		2017		98.51

		2016		98.53

		2015		98.55

		2014		98.57

		2013		98.59

		2012		98.61

		2011		98.63

		2010		98.65

		2009		98.66

		2008		98.68

		2007		98.69

		2006		98.69

		2005		98.69

		2004		98.68

		2003		98.67

		2002		98.65

		2001		98.64

		2000		98.62

		1999		98.6

		1998		98.58

		1997		98.56

		1996		98.55

		1995		98.54

		1994		98.53

		1993		98.52

		1992		98.51

		1991		98.51

		1990		98.5

		1989		98.49

		1988		98.47

		1987		98.46

		1986		98.45

		1985		98.45

		1984		98.44

		1983		98.44

		1982		98.45

		1981		98.47

		1980		98.49

		1979		98.51

		1978		98.55

		1977		98.58

		1976		98.61

		1975		98.63

		1974		98.65

		1973		98.67

		1972		98.68

		1971		98.68

		1970		98.69

		1969		98.68

		1968		98.68

		1967		98.67

		1966		98.67

		1965		98.67

		1964		98.67

		1963		98.67

		1962		98.68

		1961		98.68

		1960		98.68

		1959		98.68

		1958		98.67

		1957		98.67

		1956		98.66

		1955		98.65

		1954		98.64

		1953		98.63

		1952		98.62

		1951		98.61

		1950		98.61

		1949		98.61

		1948		98.6

		1947		98.6

		1946		98.6

		1945		98.6

		1944		98.6

		1943		98.6

		1942		98.6

		1941		98.6

		1940		98.59

		1939		98.59

		1938		98.58

		1937		98.58

		1936		98.57

		1935		98.56

		1934		98.56

		1933		98.55

		1932		98.55

		1931		98.54

		1930		98.54

		1929		98.53

		1928		98.52

		1927		98.52

		1926		98.51

		1925		98.5

		1924		98.49

		1923		98.48

		1922		98.47

		1921		98.46

		1920		98.45

		1919		98.44

		1918		98.43

		1917		98.42

		1916		98.42

		1915		98.41

		1914		98.41

		1913		98.4

		1912		98.4

		1911		98.39

		1910		98.39

		1909		98.38

		1908		98.38

		1907		98.37

		1906		98.36

		1905		98.35

		1904		98.33

		1903		98.32

		1902		98.31

		1901		98.29

		1900		98.28

		1899		98.26

		1898		98.25

		1897		98.24

		1896		98.23

		1895		98.23

		1894		98.22

		1893		98.22

		1892		98.22

		1891		98.21

		1890		98.21

		1889		98.21

		1888		98.21

		1887		98.2

		1886		98.2

		1885		98.19

		1884		98.19

		1883		98.18

		1882		98.17

		1881		98.16

		1880		98.16

		1879		98.15

		1878		98.14

		1877		98.13

		1876		98.12

		1875		98.1

		1874		98.09

		1873		98.08

		1872		98.07

		1871		98.07

		1870		98.06

		1869		98.05

		1868		98.04

		1867		98.03

		1866		98.02

		1865		98.01

		1864		97.99

		1863		97.98

		1862		97.97

		1861		97.95

		1860		97.93

		1859		97.92

		1858		97.9

		1857		97.89

		1856		97.87

		1855		97.86

		1854		97.85

		1853		97.83

		1852		97.82

		1851		97.81

		1850		97.8

		1849		97.79

		1848		97.78

		1847		97.77

		1846		97.76

		1845		97.75

		1844		97.74

		1843		97.72

		1842		97.71

		1841		97.7

		1840		97.69

		1839		97.68

		1838		97.67

		1837		97.66

		1836		97.65

		1835		97.65

		1834		97.64

		1833		97.63

		1832		97.62

		1831		97.61

		1830		97.6

		1829		97.59

		1828		97.57

		1827		97.55

		1826		97.54

		1825		97.52

		1824		97.5

		1823		97.48

		1822		97.46

		1821		97.44

		1820		97.42

		1819		97.4

		1818		97.38

		1817		97.36

		1816		97.35

		1815		97.33

		1814		97.32

		1813		97.31

		1812		97.3

		1811		97.28

		1810		97.27

		1809		97.26

		1808		97.25

		1807		97.24

		1806		97.23

		1805		97.22

		1804		97.21

		1803		97.19

		1802		97.18

		1801		97.16

		1800		97.13

		1799		97.11

		1798		97.07

		1797		97.04

		1796		97

		1795		96.96

		1794		96.91

		1793		96.87

		1792		96.82

		1791		96.77

		1790		96.73

		1789		96.69

		1788		96.66

		1787		96.63

		1786		96.62

		1785		96.61

		1784		96.61

		1783		96.63

		1782		96.65

		1781		96.68

		1780		96.72

		1779		96.76

		1778		96.81

		1777		96.86

		1776		96.9

		1775		96.95

		1774		97

		1773		97.04

		1772		97.08

		1771		97.12

		1770		97.16

		1769		97.19

		1768		97.22

		1767		97.25

		1766		97.28

		1765		97.3

		1764		97.33

		1763		97.35

		1762		97.37

		1761		97.38

		1760		97.4

		1759		97.41

		1758		97.42

		1757		97.43

		1756		97.43

		1755		97.43

		1754		97.43

		1753		97.43

		1752		97.42

		1751		97.4

		1750		97.39

		1749		97.36

		1748		97.34

		1747		97.3

		1746		97.27

		1745		97.22

		1744		97.17

		1743		97.12

		1742		97.06

		1741		96.98

		1740		96.9

		1739		96.82

		1738		96.72

		1737		96.61

		1736		96.49

		1735		96.35

		1734		96.19

		1733		96.01

		1732		95.81

		1731		95.57

		1730		95.31

		1729		95.01

		1728		94.66

		1727		94.25

		1726		93.78

		1725		93.23

		1724		92.6

		1723		91.87

		1722		91.06

		1721		90.15

		1720		89.15

		1719		88.05

		1718		86.86

		1717		85.59

		1716		84.25

		1715		82.85

		1714		81.39

		1713		79.88

		1712		78.32

		1711		76.72

		1710		75.09

		1709		73.43

		1708		71.77

		1707		70.11

		1706		68.49

		1705		66.92

		1704		65.45

		1703		64.1

		1702		62.88

		1701		61.82

		1700		60.93

		1699		60.24

		1698		59.75

		1697		59.44

		1696		59.32

		1695		59.34

		1694		59.5

		1693		59.79

		1692		60.19

		1691		60.71

		1690		61.32

		1689		62.04

		1688		62.84

		1687		63.75

		1686		64.76

		1685		65.89

		1684		67.15

		1683		68.5

		1682		69.95

		1681		71.46

		1680		73.04

		1679		74.64

		1678		76.26

		1677		77.86

		1676		79.43

		1675		80.93

		1674		82.35

		1673		83.66

		1672		84.88

		1671		85.99

		1670		87

		1669		87.91

		1668		88.72

		1667		89.44

		1666		90.07

		1665		90.63

		1664		91.12

		1663		91.57

		1662		91.96

		1661		92.32

		1660		92.64

		1659		92.92

		1658		93.18

		1657		93.41

		1656		93.63

		1655		93.82

		1654		94.01

		1653		94.17

		1652		94.33

		1651		94.48

		1650		94.62

		1649		94.75

		1648		94.87

		1647		94.99

		1646		95.11

		1645		95.22

		1644		95.32

		1643		95.42

		1642		95.52

		1641		95.62

		1640		95.71

		1639		95.8

		1638		95.89

		1637		95.97

		1636		96.05

		1635		96.12

		1634		96.2

		1633		96.27

		1632		96.34

		1631		96.4

		1630		96.47

		1629		96.53

		1628		96.59

		1627		96.65

		1626		96.71

		1625		96.77

		1624		96.82

		1623		96.88

		1622		96.93

		1621		96.98

		1620		97.03

		1619		97.08

		1618		97.13

		1617		97.18

		1616		97.23

		1615		97.28

		1614		97.32

		1613		97.37

		1612		97.41

		1611		97.45

		1610		97.49

		1609		97.52

		1608		97.56

		1607		97.59

		1606		97.62

		1605		97.64

		1604		97.67

		1603		97.69

		1602		97.71

		1601		97.73

		1600		97.74

		1599		97.76

		1598		97.77

		1597		97.78

		1596		97.8

		1595		97.81

		1594		97.83

		1593		97.84

		1592		97.86

		1591		97.88

		1590		97.89

		1589		97.91

		1588		97.93

		1587		97.94

		1586		97.96

		1585		97.97

		1584		97.98

		1583		98

		1582		98

		1581		98.01

		1580		98.02

		1579		98.02

		1578		98.03

		1577		98.03

		1576		98.03

		1575		98.03

		1574		98.03

		1573		98.04

		1572		98.04

		1571		98.04

		1570		98.04

		1569		98.04

		1568		98.04

		1567		98.05

		1566		98.05

		1565		98.06

		1564		98.06

		1563		98.07

		1562		98.08

		1561		98.09

		1560		98.09

		1559		98.1

		1558		98.11

		1557		98.11

		1556		98.12

		1555		98.13

		1554		98.13

		1553		98.14

		1552		98.14

		1551		98.15

		1550		98.16

		1549		98.16

		1548		98.17

		1547		98.17

		1546		98.18

		1545		98.18

		1544		98.19

		1543		98.19

		1542		98.2

		1541		98.2

		1540		98.21

		1539		98.21

		1538		98.22

		1537		98.22

		1536		98.22

		1535		98.22

		1534		98.22

		1533		98.22

		1532		98.22

		1531		98.21

		1530		98.21

		1529		98.2

		1528		98.19

		1527		98.18

		1526		98.18

		1525		98.17

		1524		98.16

		1523		98.15

		1522		98.14

		1521		98.13

		1520		98.11

		1519		98.11

		1518		98.1

		1517		98.09

		1516		98.08

		1515		98.07

		1514		98.06

		1513		98.06

		1512		98.05

		1511		98.05

		1510		98.04

		1509		98.04

		1508		98.03

		1507		98.03

		1506		98.03

		1505		98.02

		1504		98.02

		1503		98.01

		1502		98

		1501		98

		1500		97.99

		1499		97.98

		1498		97.97

		1497		97.95

		1496		97.94

		1495		97.92

		1494		97.9

		1493		97.88

		1492		97.86

		1491		97.83

		1490		97.79

		1489		97.75

		1488		97.7

		1487		97.63

		1486		97.54

		1485		97.41

		1484		97.23

		1483		96.97

		1482		96.6

		1481		96.09

		1480		95.45

		1479		94.69

		1478		93.84

		1477		92.91

		1476		91.93

		1475		90.92

		1474		89.92

		1473		88.98

		1472		88.16

		1471		87.54

		1470		87.1

		1469		86.84

		1468		86.72

		1467		86.7

		1466		86.78

		1465		86.95

		1464		87.2

		1463		87.52

		1462		87.88

		1461		88.23

		1460		88.57

		1459		88.9

		1458		89.23

		1457		89.57

		1456		89.92

		1455		90.25

		1454		90.54

		1453		90.79

		1452		90.98

		1451		91.11

		1450		91.19

		1449		91.21

		1448		91.17

		1447		91.07

		1446		90.91

		1445		90.71

		1444		90.46

		1443		90.16

		1442		89.81

		1441		89.42

		1440		88.98

		1439		88.5

		1438		87.98

		1437		87.44

		1436		86.88

		1435		86.34

		1434		85.83

		1433		85.37

		1432		84.98

		1431		84.7

		1430		84.52

		1429		84.47

		1428		84.54

		1427		84.73

		1426		85.03

		1425		85.41

		1424		85.84

		1423		86.28

		1422		86.7

		1421		87.06

		1420		87.35

		1419		87.56

		1418		87.66

		1417		87.66

		1416		87.59

		1415		87.45

		1414		87.29

		1413		87.14

		1412		87.04

		1411		87.02

		1410		87.1

		1409		87.31

		1408		87.63

		1407		88.07

		1406		88.61

		1405		89.24

		1404		89.92

		1403		90.64

		1402		91.35

		1401		92.04

		1400		92.69

		1399		93.28

		1398		93.81

		1397		94.28

		1396		94.68

		1395		95.02

		1394		95.3

		1393		95.53

		1392		95.72

		1391		95.87

		1390		95.99

		1389		96.08

		1388		96.14

		1387		96.18

		1386		96.2

		1385		96.19

		1384		96.15

		1383		96.1

		1382		96.02

		1381		95.93

		1380		95.82

		1379		95.7

		1378		95.58

		1377		95.46

		1376		95.34

		1375		95.23

		1374		95.12

		1373		95.03

		1372		94.95

		1371		94.88

		1370		94.8

		1369		94.72

		1368		94.62

		1367		94.49

		1366		94.35

		1365		94.18

		1364		93.98

		1363		93.77

		1362		93.54

		1361		93.29

		1360		93.04

		1359		92.79

		1358		92.55

		1357		92.33

		1356		92.13

		1355		91.97

		1354		91.84

		1353		91.75

		1352		91.7

		1351		91.71

		1350		91.77

		1349		91.88

		1348		92.04

		1347		92.25

		1346		92.49

		1345		92.74

		1344		93.01

		1343		93.26

		1342		93.47

		1341		93.63

		1340		93.72

		1339		93.73

		1338		93.65

		1337		93.49

		1336		93.26

		1335		92.98

		1334		92.66

		1333		92.34

		1332		92.04

		1331		91.78

		1330		91.59

		1329		91.47

		1328		91.44

		1327		91.48

		1326		91.56

		1325		91.68

		1324		91.81

		1323		91.89

		1322		91.92

		1321		91.84

		1320		91.64

		1319		91.29

		1318		90.79

		1317		90.14

		1316		89.35

		1315		88.46

		1314		87.5

		1313		86.5

		1312		85.5

		1311		84.55

		1310		83.69

		1309		82.96

		1308		82.38

		1307		81.95

		1306		81.67

		1305		81.53

		1304		81.5

		1303		81.56

		1302		81.66

		1301		81.79

		1300		81.9

		1299		81.97

		1298		81.96

		1297		81.86

		1296		81.65

		1295		81.35

		1294		80.98

		1293		80.57

		1292		80.15

		1291		79.75

		1290		79.39

		1289		79.12

		1288		78.98

		1287		79

		1286		79.21

		1285		79.62

		1284		80.23

		1283		81

		1282		81.9

		1281		82.91

		1280		83.97

		1279		85.05

		1278		86.11

		1277		87.1

		1276		87.99

		1275		88.75

		1274		89.34

		1273		89.75

		1272		89.97

		1271		90.01

		1270		89.89

		1269		89.63

		1268		89.25

		1267		88.79

		1266		88.3

		1265		87.82

		1264		87.4

		1263		87.09

		1262		86.94

		1261		86.97

		1260		87.19

		1259		87.58

		1258		88.12

		1257		88.77

		1256		89.49

		1255		90.26

		1254		91.01

		1253		91.72

		1252		92.34

		1251		92.84

		1250		93.19

		1249		93.38

		1248		93.38

		1247		93.2

		1246		92.83

		1245		92.3

		1244		91.62

		1243		90.84

		1242		89.99

		1241		89.12

		1240		88.29

		1239		87.55

		1238		86.98

		1237		86.63

		1236		86.52

		1235		86.65

		1234		86.99

		1233		87.52

		1232		88.18

		1231		88.94

		1230		89.74

		1229		90.53

		1228		91.24

		1227		91.85

		1226		92.3

		1225		92.58

		1224		92.69

		1223		92.62

		1222		92.39

		1221		92.02

		1220		91.53

		1219		90.95

		1218		90.31

		1217		89.65

		1216		89.03

		1215		88.48

		1214		88.06

		1213		87.8

		1212		87.72

		1211		87.82

		1210		88.09

		1209		88.51

		1208		89.06

		1207		89.7

		1206		90.39

		1205		91.08

		1204		91.73

		1203		92.29

		1202		92.71

		1201		92.97

		1200		93.04

		1199		92.94

		1198		92.68

		1197		92.28

		1196		91.79

		1195		91.25

		1194		90.68

		1193		90.16

		1192		89.73

		1191		89.45

		1190		89.35

		1189		89.45

		1188		89.74

		1187		90.18

		1186		90.73

		1185		91.36

		1184		92.03

		1183		92.71

		1182		93.38

		1181		93.98

		1180		94.51

		1179		94.96

		1178		95.31

		1177		95.6

		1176		95.84

		1175		96.03

		1174		96.19

		1173		96.32

		1172		96.44

		1171		96.54

		1170		96.64

		1169		96.72

		1168		96.79

		1167		96.86

		1166		96.92

		1165		96.98

		1164		97.03

		1163		97.08

		1162		97.12

		1161		97.17

		1160		97.21

		1159		97.24

		1158		97.28

		1157		97.31

		1156		97.34

		1155		97.37

		1154		97.39

		1153		97.42

		1152		97.44

		1151		97.46

		1150		97.48

		1149		97.5

		1148		97.52

		1147		97.54

		1146		97.55

		1145		97.57

		1144		97.58

		1143		97.59

		1142		97.61

		1141		97.61

		1140		97.62

		1139		97.62

		1138		97.61

		1137		97.59

		1136		97.56

		1135		97.52

		1134		97.46

		1133		97.38

		1132		97.29

		1131		97.19

		1130		97.08

		1129		96.96

		1128		96.86

		1127		96.76

		1126		96.68

		1125		96.62

		1124		96.59

		1123		96.59

		1122		96.62

		1121		96.68

		1120		96.76

		1119		96.86

		1118		96.96

		1117		97.07

		1116		97.18

		1115		97.29

		1114		97.38

		1113		97.46

		1112		97.52

		1111		97.58

		1110		97.62

		1109		97.65

		1108		97.68

		1107		97.69

		1106		97.68

		1105		97.65

		1104		97.58

		1103		97.46

		1102		97.29

		1101		97.07

		1100		96.8

		1099		96.49

		1098		96.16

		1097		95.82

		1096		95.48

		1095		95.18

		1094		94.94

		1093		94.78

		1092		94.72

		1091		94.76

		1090		94.9

		1089		95.11

		1088		95.38

		1087		95.69

		1086		96.02

		1085		96.36

		1084		96.67

		1083		96.96

		1082		97.2

		1081		97.4

		1080		97.56

		1079		97.67

		1078		97.76

		1077		97.83

		1076		97.87

		1075		97.91

		1074		97.93

		1073		97.95

		1072		97.95

		1071		97.95

		1070		97.95

		1069		97.94

		1068		97.93

		1067		97.92

		1066		97.91

		1065		97.91

		1064		97.9

		1063		97.89

		1062		97.89

		1061		97.88

		1060		97.88

		1059		97.87

		1058		97.87

		1057		97.86

		1056		97.85

		1055		97.84

		1054		97.83

		1053		97.81

		1052		97.79

		1051		97.77

		1050		97.74

		1049		97.7

		1048		97.65

		1047		97.6

		1046		97.53

		1045		97.45

		1044		97.38

		1043		97.3

		1042		97.22

		1041		97.14

		1040		97.08

		1039		97.03

		1038		97

		1037		96.99

		1036		96.98

		1035		96.99

		1034		97.01

		1033		97.03

		1032		97.05

		1031		97.07

		1030		97.08

		1029		97.08

		1028		97.08

		1027		97.06

		1026		97.05

		1025		97.02

		1024		97

		1023		96.97

		1022		96.94

		1021		96.92

		1020		96.89

		1019		96.87

		1018		96.84

		1017		96.81

		1016		96.78

		1015		96.74

		1014		96.7

		1013		96.66

		1012		96.61

		1011		96.55

		1010		96.49

		1009		96.42

		1008		96.35

		1007		96.27

		1006		96.19

		1005		96.11

		1004		96.03

		1003		95.96

		1002		95.89

		1001		95.83

		1000		95.78

		999		95.74

		998		95.72

		997		95.7

		996		95.68

		995		95.66

		994		95.64

		993		95.6

		992		95.56

		991		95.5

		990		95.44

		989		95.37

		988		95.29

		987		95.2

		986		95.12

		985		95.04

		984		94.96

		983		94.89

		982		94.81

		981		94.72

		980		94.62

		979		94.51

		978		94.37

		977		94.21

		976		94.03

		975		93.81

		974		93.56

		973		93.28

		972		92.98

		971		92.65

		970		92.3

		969		91.94

		968		91.57

		967		91.2

		966		90.81

		965		90.42

		964		90.03

		963		89.64

		962		89.25

		961		88.86

		960		88.47

		959		88.08

		958		87.69

		957		87.29

		956		86.89

		955		86.48

		954		86.06

		953		85.63

		952		85.19

		951		84.72

		950		84.25

		949		83.75

		948		83.25

		947		82.74

		946		82.24

		945		81.76

		944		81.31

		943		80.9

		942		80.54

		941		80.25

		940		80.04

		939		79.92

		938		79.89

		937		79.96

		936		80.12

		935		80.38

		934		80.72

		933		81.13

		932		81.61

		931		82.15

		930		82.73

		929		83.34

		928		83.97

		927		84.6

		926		85.22

		925		85.83

		924		86.42

		923		86.96

		922		87.46

		921		87.91

		920		88.3

		919		88.63

		918		88.89

		917		89.1

		916		89.24

		915		89.34

		914		89.41

		913		89.45

		912		89.48

		911		89.52

		910		89.57

		909		89.65

		908		89.76

		907		89.91

		906		90.09

		905		90.29

		904		90.51

		903		90.72

		902		90.91

		901		91.08

		900		91.21

		899		91.3

		898		91.34

		897		91.33

		896		91.29

		895		91.22

		894		91.13

		893		91.04

		892		90.98

		891		90.93

		890		90.92

		889		90.95

		888		91.03

		887		91.16

		886		91.34

		885		91.56

		884		91.81

		883		92.07

		882		92.34

		881		92.62

		880		92.88

		879		93.14

		878		93.38

		877		93.6

		876		93.8

		875		93.98

		874		94.14

		873		94.28

		872		94.42

		871		94.55

		870		94.67

		869		94.78

		868		94.88

		867		94.98

		866		95.07

		865		95.16

		864		95.25

		863		95.34

		862		95.42

		861		95.51

		860		95.6

		859		95.69

		858		95.78

		857		95.88

		856		95.98

		855		96.07

		854		96.17

		853		96.26

		852		96.35

		851		96.43

		850		96.51

		849		96.59

		848		96.66

		847		96.73

		846		96.79

		845		96.85

		844		96.91

		843		96.96

		842		97.01

		841		97.06

		840		97.1

		839		97.14

		838		97.18

		837		97.22

		836		97.25

		835		97.28

		834		97.31

		833		97.34

		832		97.36

		831		97.38

		830		97.39

		829		97.39

		828		97.38

		827		97.35

		826		97.3

		825		97.23

		824		97.12

		823		96.98

		822		96.82

		821		96.65

		820		96.47

		819		96.3

		818		96.15

		817		96.02

		816		95.94

		815		95.91

		814		95.95

		813		96.06

		812		96.22

		811		96.41

		810		96.63

		809		96.87

		808		97.1

		807		97.32

		806		97.53

		805		97.7

		804		97.85

		803		97.96

		802		98.04

		801		98.11

		800		98.15

		799		98.19

		798		98.22

		797		98.24

		796		98.25

		795		98.26

		794		98.26

		793		98.24

		792		98.22

		791		98.18

		790		98.12

		789		98.05

		788		97.97

		787		97.89

		786		97.8

		785		97.72

		784		97.65

		783		97.6

		782		97.56

		781		97.56

		780		97.58

		779		97.63

		778		97.71

		777		97.79

		776		97.88

		775		97.97

		774		98.06

		773		98.14

		772		98.21

		771		98.27

		770		98.3

		769		98.32

		768		98.32

		767		98.3

		766		98.27

		765		98.2

		764		98.11

		763		97.98

		762		97.8

		761		97.6

		760		97.36

		759		97.11

		758		96.86

		757		96.62

		756		96.41

		755		96.23

		754		96.11

		753		96.07

		752		96.1

		751		96.21

		750		96.38

		749		96.58

		748		96.79

		747		96.99

		746		97.18

		745		97.33

		744		97.43

		743		97.48

		742		97.45

		741		97.34

		740		97.14

		739		96.84

		738		96.43

		737		95.89

		736		95.23

		735		94.44

		734		93.56

		733		92.6

		732		91.56

		731		90.49

		730		89.4

		729		88.36

		728		87.41

		727		86.63

		726		86.06

		725		85.71

		724		85.58

		723		85.66

		722		85.94

		721		86.42

		720		87.09

		719		87.92

		718		88.87

		717		89.88

		716		90.87

		715		91.82

		714		92.7

		713		93.51

		712		94.22

		711		94.84

		710		95.33

		709		95.71

		708		95.97

		707		96.14

		706		96.22

		705		96.23

		704		96.18

		703		96.07

		702		95.9

		701		95.66

		700		95.35

		699		94.97

		698		94.51

		697		93.99

		696		93.4

		695		92.77

		694		92.11

		693		91.45

		692		90.8

		691		90.2

		690		89.67

		689		89.24

		688		88.91

		687		88.71

		686		88.63

		685		88.66

		684		88.79

		683		89.02

		682		89.31

		681		89.64

		680		90

		679		90.37

		678		90.73

		677		91.07

		676		91.39

		675		91.68

		674		91.94

		673		92.19

		672		92.42

		671		92.65

		670		92.87

		669		93.09

		668		93.32

		667		93.56

		666		93.81

		665		94.07

		664		94.33

		663		94.6

		662		94.87

		661		95.13

		660		95.39

		659		95.64

		658		95.87

		657		96.1

		656		96.3

		655		96.49

		654		96.67

		653		96.83

		652		96.97

		651		97.1

		650		97.21

		649		97.31

		648		97.39

		647		97.47

		646		97.52

		645		97.57

		644		97.61

		643		97.65

		642		97.68

		641		97.7

		640		97.73

		639		97.75

		638		97.78

		637		97.81

		636		97.84

		635		97.87

		634		97.91

		633		97.95

		632		97.99

		631		98.03

		630		98.07

		629		98.11

		628		98.15

		627		98.19

		626		98.22

		625		98.26

		624		98.29

		623		98.32

		622		98.35

		621		98.37

		620		98.4

		619		98.42

		618		98.43

		617		98.45

		616		98.46

		615		98.48

		614		98.49

		613		98.5

		612		98.52

		611		98.54

		610		98.55

		609		98.57

		608		98.59

		607		98.6

		606		98.62

		605		98.64

		604		98.65

		603		98.66

		602		98.67

		601		98.68

		600		98.69

		599		98.69

		598		98.7

		597		98.7

		596		98.71

		595		98.71

		594		98.71

		593		98.71

		592		98.7

		591		98.7

		590		98.69

		589		98.68

		588		98.67

		587		98.65

		586		98.63

		585		98.6

		584		98.57

		583		98.53

		582		98.48

		581		98.42

		580		98.35

		579		98.28

		578		98.19

		577		98.08

		576		97.97

		575		97.83

		574		97.68

		573		97.52

		572		97.33

		571		97.12

		570		96.9

		569		96.66

		568		96.39

		567		96.11

		566		95.81

		565		95.48

		564		95.13

		563		94.76

		562		94.37

		561		93.96

		560		93.53

		559		93.09

		558		92.64

		557		92.18

		556		91.73

		555		91.3

		554		90.9

		553		90.55

		552		90.25

		551		90.02

		550		89.87

		549		89.81

		548		89.84

		547		89.97

		546		90.2

		545		90.52

		544		90.92

		543		91.39

		542		91.91

		541		92.47

		540		93.04

		539		93.62

		538		94.18

		537		94.72

		536		95.22

		535		95.68

		534		96.1

		533		96.46

		532		96.78

		531		97.05

		530		97.28

		529		97.47

		528		97.64

		527		97.78

		526		97.9

		525		98

		524		98.09

		523		98.17

		522		98.24

		521		98.3

		520		98.35

		519		98.39

		518		98.42

		517		98.44

		516		98.44

		515		98.42

		514		98.37

		513		98.29

		512		98.16

		511		97.99

		510		97.75

		509		97.45

		508		97.08

		507		96.67

		506		96.21

		505		95.73

		504		95.24

		503		94.78

		502		94.37

		501		94.04

		500		93.82

		499		93.71

		498		93.72

		497		93.85

		496		94.09

		495		94.4

		494		94.77

		493		95.17

		492		95.58

		491		95.98

		490		96.35

		489		96.67

		488		96.95

		487		97.17

		486		97.35

		485		97.5

		484		97.62

		483		97.71

		482		97.8

		481		97.87

		480		97.94

		479		98.01

		478		98.07

		477		98.14

		476		98.2

		475		98.26

		474		98.32

		473		98.38

		472		98.44

		471		98.49

		470		98.54

		469		98.58

		468		98.61

		467		98.63

		466		98.65

		465		98.66

		464		98.66

		463		98.66

		462		98.65

		461		98.63

		460		98.61

		459		98.58

		458		98.54

		457		98.49

		456		98.44

		455		98.38

		454		98.3

		453		98.2

		452		98.09

		451		97.96

		450		97.79

		449		97.58

		448		97.32

		447		97.01

		446		96.63

		445		96.18

		444		95.67

		443		95.12

		442		94.55

		441		93.97

		440		93.43

		439		92.94

		438		92.55

		437		92.28

		436		92.15

		435		92.18

		434		92.36

		433		92.68

		432		93.12

		431		93.63

		430		94.19

		429		94.77

		428		95.34

		427		95.87

		426		96.33

		425		96.71

		424		96.99

		423		97.19

		422		97.31

		421		97.36

		420		97.38

		419		97.37

		418		97.35

		417		97.34

		416		97.34

		415		97.37

		414		97.43

		413		97.52

		412		97.65

		411		97.8

		410		97.96

		409		98.13

		408		98.28

		407		98.42

		406		98.54

		405		98.62

		404		98.69

		403		98.72

		402		98.73

		401		98.72

		400		98.71
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		nm		A

		1400		0.6646

		1399		0.6648

		1398		0.6649

		1397		0.6651

		1396		0.6652

		1395		0.6653

		1394		0.6653

		1393		0.6654

		1392		0.6655

		1391		0.6655

		1390		0.6656

		1389		0.6656

		1388		0.6656

		1387		0.6656

		1386		0.6656

		1385		0.6656

		1384		0.6656

		1383		0.6656

		1382		0.6656

		1381		0.6656

		1380		0.6656

		1379		0.6657

		1378		0.6657

		1377		0.6658

		1376		0.6659

		1375		0.666

		1374		0.6661

		1373		0.6662

		1372		0.6663

		1371		0.6664

		1370		0.6664

		1369		0.6665

		1368		0.6666

		1367		0.6667

		1366		0.6668

		1365		0.6669

		1364		0.667

		1363		0.6671

		1362		0.6671

		1361		0.6672

		1360		0.6673

		1359		0.6674

		1358		0.6675

		1357		0.6676

		1356		0.6677

		1355		0.6678

		1354		0.6679

		1353		0.6681

		1352		0.6683

		1351		0.6684

		1350		0.6686

		1349		0.6688

		1348		0.669

		1347		0.6692

		1346		0.6694

		1345		0.6696

		1344		0.6698

		1343		0.67

		1342		0.6702

		1341		0.6704

		1340		0.6706

		1339		0.6708

		1338		0.6709

		1337		0.6711

		1336		0.6712

		1335		0.6714

		1334		0.6715

		1333		0.6716

		1332		0.6718

		1331		0.6719

		1330		0.672

		1329		0.6721

		1328		0.6722

		1327		0.6723

		1326		0.6724

		1325		0.6725

		1324		0.6726

		1323		0.6727

		1322		0.6728

		1321		0.6728

		1320		0.6729

		1319		0.673

		1318		0.673

		1317		0.6731

		1316		0.6732

		1315		0.6732

		1314		0.6733

		1313		0.6734

		1312		0.6734

		1311		0.6735

		1310		0.6735

		1309		0.6736

		1308		0.6737

		1307		0.6738

		1306		0.6739

		1305		0.674

		1304		0.6741

		1303		0.6742

		1302		0.6743

		1301		0.6744

		1300		0.6745

		1299		0.6746

		1298		0.6747

		1297		0.6749

		1296		0.675

		1295		0.6751

		1294		0.6752

		1293		0.6754

		1292		0.6755

		1291		0.6756

		1290		0.6757

		1289		0.6758

		1288		0.6759

		1287		0.676

		1286		0.6761

		1285		0.6762

		1284		0.6763

		1283		0.6764

		1282		0.6765

		1281		0.6766

		1280		0.6767

		1279		0.6768

		1278		0.6769

		1277		0.677

		1276		0.6771

		1275		0.6772

		1274		0.6773

		1273		0.6774

		1272		0.6775

		1271		0.6776

		1270		0.6776

		1269		0.6777

		1268		0.6778

		1267		0.6779

		1266		0.6779

		1265		0.678

		1264		0.6781

		1263		0.6781

		1262		0.6782

		1261		0.6783

		1260		0.6784

		1259		0.6784

		1258		0.6785

		1257		0.6786

		1256		0.6787

		1255		0.6788

		1254		0.6789

		1253		0.679

		1252		0.6792

		1251		0.6793

		1250		0.6794

		1249		0.6796

		1248		0.6797

		1247		0.6799

		1246		0.6801

		1245		0.6802

		1244		0.6804

		1243		0.6806

		1242		0.6808

		1241		0.681

		1240		0.6812

		1239		0.6814

		1238		0.6816

		1237		0.6819

		1236		0.6821

		1235		0.6823

		1234		0.6826

		1233		0.6829

		1232		0.6831

		1231		0.6834

		1230		0.6837

		1229		0.684

		1228		0.6843

		1227		0.6847

		1226		0.685

		1225		0.6853

		1224		0.6856

		1223		0.6859

		1222		0.6862

		1221		0.6865

		1220		0.6868

		1219		0.6871

		1218		0.6873

		1217		0.6876

		1216		0.6878

		1215		0.688

		1214		0.6881

		1213		0.6883

		1212		0.6884

		1211		0.6884

		1210		0.6885

		1209		0.6885

		1208		0.6885

		1207		0.6885

		1206		0.6885

		1205		0.6884

		1204		0.6884

		1203		0.6883

		1202		0.6882

		1201		0.688

		1200		0.6879

		1199		0.6877

		1198		0.6876

		1197		0.6874

		1196		0.6872

		1195		0.6871

		1194		0.6869

		1193		0.6867

		1192		0.6866

		1191		0.6864

		1190		0.6862

		1189		0.686

		1188		0.6859

		1187		0.6857

		1186		0.6855

		1185		0.6854

		1184		0.6853

		1183		0.6851

		1182		0.685

		1181		0.6849

		1180		0.6847

		1179		0.6846

		1178		0.6845

		1177		0.6844

		1176		0.6843

		1175		0.6842

		1174		0.6841

		1173		0.6841

		1172		0.684

		1171		0.6839

		1170		0.6838

		1169		0.6837

		1168		0.6837

		1167		0.6836

		1166		0.6835

		1165		0.6835

		1164		0.6834

		1163		0.6833

		1162		0.6832

		1161		0.6831

		1160		0.6831

		1159		0.683

		1158		0.6829

		1157		0.6828

		1156		0.6827

		1155		0.6827

		1154		0.6826

		1153		0.6826

		1152		0.6825

		1151		0.6825

		1150		0.6824

		1149		0.6824

		1148		0.6824

		1147		0.6824

		1146		0.6823

		1145		0.6823

		1144		0.6823

		1143		0.6823

		1142		0.6823

		1141		0.6824

		1140		0.6824

		1139		0.6824

		1138		0.6823

		1137		0.6823

		1136		0.6823

		1135		0.6823

		1134		0.6823

		1133		0.6823

		1132		0.6823

		1131		0.6823

		1130		0.6823

		1129		0.6823

		1128		0.6822

		1127		0.6822

		1126		0.6822

		1125		0.6822

		1124		0.6822

		1123		0.6821

		1122		0.6821

		1121		0.6821

		1120		0.6821

		1119		0.6821

		1118		0.6821

		1117		0.6821

		1116		0.6821

		1115		0.6821

		1114		0.6821

		1113		0.6821

		1112		0.6821

		1111		0.6821

		1110		0.6821

		1109		0.6821

		1108		0.6822

		1107		0.6822

		1106		0.6822

		1105		0.6822

		1104		0.6822

		1103		0.6823

		1102		0.6823

		1101		0.6823

		1100		0.6823

		1099		0.6823

		1098		0.6823

		1097		0.6824

		1096		0.6824

		1095		0.6824

		1094		0.6823

		1093		0.6823

		1092		0.6823

		1091		0.6823

		1090		0.6823

		1089		0.6823

		1088		0.6823

		1087		0.6823

		1086		0.6823

		1085		0.6822

		1084		0.6822

		1083		0.6822

		1082		0.6822

		1081		0.6822

		1080		0.6821

		1079		0.6821

		1078		0.6821

		1077		0.6821

		1076		0.6821

		1075		0.6822

		1074		0.6821

		1073		0.6821

		1072		0.6821

		1071		0.6821

		1070		0.6821

		1069		0.6821

		1068		0.6822

		1067		0.6822

		1066		0.6822

		1065		0.6822

		1064		0.6822

		1063		0.6823

		1062		0.6823

		1061		0.6823

		1060		0.6823

		1059		0.6823

		1058		0.6823

		1057		0.6824

		1056		0.6824

		1055		0.6825

		1054		0.6825

		1053		0.6826

		1052		0.6826

		1051		0.6826

		1050		0.6827

		1049		0.6827

		1048		0.6828

		1047		0.6828

		1046		0.6828

		1045		0.6829

		1044		0.6829

		1043		0.6829

		1042		0.6829

		1041		0.683

		1040		0.683

		1039		0.683

		1038		0.683

		1037		0.6829

		1036		0.6829

		1035		0.6829

		1034		0.6829

		1033		0.6829

		1032		0.6829

		1031		0.6829

		1030		0.6829

		1029		0.6829

		1028		0.6829

		1027		0.6829

		1026		0.6829

		1025		0.6829

		1024		0.6829

		1023		0.6828

		1022		0.6828

		1021		0.6828

		1020		0.6828

		1019		0.6828

		1018		0.6828

		1017		0.6828

		1016		0.6827

		1015		0.6827

		1014		0.6827

		1013		0.6827

		1012		0.6827

		1011		0.6826

		1010		0.6826

		1009		0.6826

		1008		0.6825

		1007		0.6825

		1006		0.6825

		1005		0.6824

		1004		0.6824

		1003		0.6823

		1002		0.6823

		1001		0.6822

		1000		0.6822

		999		0.6821

		998		0.6821

		997		0.682

		996		0.6819

		995		0.6818

		994		0.6818

		993		0.6817

		992		0.6816

		991		0.6815

		990		0.6814

		989		0.6813

		988		0.6811

		987		0.681

		986		0.6808

		985		0.6807

		984		0.6805

		983		0.6803

		982		0.6802

		981		0.68

		980		0.6798

		979		0.6796

		978		0.6794

		977		0.6792

		976		0.679

		975		0.6787

		974		0.6785

		973		0.6783

		972		0.6781

		971		0.6778

		970		0.6776

		969		0.6773

		968		0.6771

		967		0.6768

		966		0.6766

		965		0.6763

		964		0.676

		963		0.6757

		962		0.6754

		961		0.6751

		960		0.6748

		959		0.6745

		958		0.6742

		957		0.6739

		956		0.6737

		955		0.6734

		954		0.6731

		953		0.6728

		952		0.6725

		951		0.6723

		950		0.6721

		949		0.6719

		948		0.6717

		947		0.6716

		946		0.6715

		945		0.6714

		944		0.6713

		943		0.6712

		942		0.6711

		941		0.6711

		940		0.6711

		939		0.6711

		938		0.6712

		937		0.6713

		936		0.6714

		935		0.6714

		934		0.6715

		933		0.6716

		932		0.6717

		931		0.6718

		930		0.6719

		929		0.6719

		928		0.672

		927		0.6721

		926		0.6722

		925		0.6723

		924		0.6724

		923		0.6725

		922		0.6725

		921		0.6726

		920		0.6727

		919		0.6728

		918		0.6729

		917		0.673

		916		0.6731

		915		0.6732

		914		0.6733

		913		0.6734

		912		0.6735

		911		0.6737

		910		0.6738

		909		0.674

		908		0.6741

		907		0.6742

		906		0.6744

		905		0.6745

		904		0.6746

		903		0.6748

		902		0.6749

		901		0.675

		900		0.6751

		899		0.6752

		898		0.6753

		897		0.6754

		896		0.6756

		895		0.6756

		894		0.6757

		893		0.6758

		892		0.6758

		891		0.6759

		890		0.676

		889		0.6761

		888		0.6762

		887		0.6763

		886		0.6764

		885		0.6765

		884		0.6766

		883		0.6767

		882		0.6768

		881		0.6769

		880		0.677

		879		0.6771

		878		0.6772

		877		0.6773

		876		0.6775

		875		0.6777

		874		0.678

		873		0.6784

		872		0.6789

		871		0.6794

		870		0.68

		869		0.6805

		868		0.6812

		867		0.6818

		866		0.6826

		865		0.6835

		864		0.6844

		863		0.6854

		862		0.6865

		861		0.6876

		860		0.6888

		859		0.6899

		858		0.691

		857		0.6919

		856		0.6928

		855		0.6936

		854		0.6943

		853		0.695

		852		0.6957

		851		0.6964

		850		0.697

		849		0.6975

		848		0.6979

		847		0.6982

		846		0.6985

		845		0.6986

		844		0.6987

		843		0.6987

		842		0.6988

		841		0.6988

		840		0.6989

		839		0.6989

		838		0.699

		837		0.699

		836		0.699

		835		0.6989

		834		0.6989

		833		0.6989

		832		0.6988

		831		0.6988

		830		0.6987

		829		0.6987

		828		0.6987

		827		0.6987

		826		0.6987

		825		0.6987

		824		0.6987

		823		0.6987

		822		0.6987

		821		0.6987

		820		0.6987

		819		0.6987

		818		0.6987

		817		0.6987

		816		0.6987

		815		0.6987

		814		0.6987

		813		0.6987

		812		0.6988

		811		0.6988

		810		0.6988

		809		0.6988

		808		0.6989

		807		0.6989

		806		0.6989

		805		0.6989

		804		0.6989

		803		0.699

		802		0.699

		801		0.6991

		800		0.6992

		799		0.6992

		798		0.6993

		797		0.6993

		796		0.6994

		795		0.6994

		794		0.6995

		793		0.6995

		792		0.6996

		791		0.6997

		790		0.6997

		789		0.6998

		788		0.6999

		787		0.6999

		786		0.6999

		785		0.7

		784		0.7

		783		0.7001

		782		0.7001

		781		0.7001

		780		0.7001

		779		0.7002

		778		0.7002

		777		0.7002

		776		0.7001

		775		0.7001

		774		0.7001

		773		0.7002

		772		0.7002

		771		0.7002

		770		0.7002

		769		0.7003

		768		0.7003

		767		0.7003

		766		0.7004

		765		0.7005

		764		0.7006

		763		0.7007

		762		0.7008

		761		0.7009

		760		0.701

		759		0.7011

		758		0.7012

		757		0.7013

		756		0.7013

		755		0.7014

		754		0.7015

		753		0.7016

		752		0.7017

		751		0.7018

		750		0.7018

		749		0.7018

		748		0.7019

		747		0.7019

		746		0.7019

		745		0.702

		744		0.702

		743		0.702

		742		0.702

		741		0.7021

		740		0.7021

		739		0.7021

		738		0.7021

		737		0.7021

		736		0.7022

		735		0.7022

		734		0.7022

		733		0.7022

		732		0.7022

		731		0.7022

		730		0.7022

		729		0.7022

		728		0.7022

		727		0.7022

		726		0.7022

		725		0.7023

		724		0.7023

		723		0.7023

		722		0.7023

		721		0.7023

		720		0.7024

		719		0.7024

		718		0.7024

		717		0.7025

		716		0.7025

		715		0.7026

		714		0.7026

		713		0.7026

		712		0.7027

		711		0.7027

		710		0.7028

		709		0.7028

		708		0.7028

		707		0.7028

		706		0.7029

		705		0.7029

		704		0.7029

		703		0.703

		702		0.703

		701		0.703

		700		0.703

		699		0.7031

		698		0.7031

		697		0.7031

		696		0.7032

		695		0.7032

		694		0.7033

		693		0.7033

		692		0.7034

		691		0.7035

		690		0.7035

		689		0.7036

		688		0.7036

		687		0.7037

		686		0.7038

		685		0.7038

		684		0.7039

		683		0.704

		682		0.704

		681		0.7041

		680		0.7041

		679		0.7042

		678		0.7042

		677		0.7043

		676		0.7043

		675		0.7043

		674		0.7044

		673		0.7044

		672		0.7045

		671		0.7045

		670		0.7046

		669		0.7046

		668		0.7046

		667		0.7047

		666		0.7047

		665		0.7047

		664		0.7048

		663		0.7048

		662		0.7048

		661		0.7048

		660		0.7049

		659		0.7049

		658		0.7049

		657		0.705

		656		0.705

		655		0.705

		654		0.705

		653		0.7051

		652		0.7051

		651		0.7051

		650		0.7052

		649		0.7052

		648		0.7053

		647		0.7053

		646		0.7053

		645		0.7054

		644		0.7054

		643		0.7054

		642		0.7054

		641		0.7055

		640		0.7055

		639		0.7055

		638		0.7056

		637		0.7056

		636		0.7056

		635		0.7057

		634		0.7057

		633		0.7057

		632		0.7057

		631		0.7058

		630		0.7058

		629		0.7059

		628		0.7059

		627		0.706

		626		0.706

		625		0.7061

		624		0.7061

		623		0.7062

		622		0.7062

		621		0.7062

		620		0.7063

		619		0.7063

		618		0.7064

		617		0.7064

		616		0.7064

		615		0.7065

		614		0.7065

		613		0.7065

		612		0.7066

		611		0.7066

		610		0.7066

		609		0.7066

		608		0.7066

		607		0.7066

		606		0.7067

		605		0.7067

		604		0.7067

		603		0.7068

		602		0.7068

		601		0.7068

		600		0.7069

		599		0.7069

		598		0.707

		597		0.707

		596		0.707

		595		0.7071

		594		0.7071

		593		0.7071

		592		0.7072

		591		0.7072

		590		0.7072

		589		0.7072

		588		0.7072

		587		0.7073

		586		0.7073

		585		0.7073

		584		0.7073

		583		0.7073

		582		0.7073

		581		0.7073

		580		0.7073

		579		0.7073

		578		0.7073

		577		0.7073

		576		0.7073

		575		0.7073

		574		0.7073

		573		0.7073

		572		0.7073

		571		0.7073

		570		0.7073

		569		0.7073

		568		0.7073

		567		0.7074

		566		0.7074

		565		0.7074

		564		0.7074

		563		0.7075

		562		0.7075

		561		0.7076

		560		0.7076

		559		0.7077

		558		0.7077

		557		0.7078

		556		0.7079

		555		0.7079

		554		0.708

		553		0.708

		552		0.7081

		551		0.7081

		550		0.7082

		549		0.7082

		548		0.7083

		547		0.7084

		546		0.7084

		545		0.7085

		544		0.7086

		543		0.7086

		542		0.7087

		541		0.7088

		540		0.7089

		539		0.709

		538		0.7092

		537		0.7093

		536		0.7095

		535		0.7097

		534		0.7099

		533		0.7101

		532		0.7103

		531		0.7106

		530		0.7108

		529		0.7111

		528		0.7114

		527		0.7117

		526		0.7121

		525		0.7124

		524		0.7127

		523		0.7131

		522		0.7134

		521		0.7137

		520		0.714

		519		0.7143

		518		0.7146

		517		0.7149

		516		0.7151

		515		0.7153

		514		0.7155

		513		0.7156

		512		0.7158

		511		0.7159

		510		0.7159

		509		0.716

		508		0.7159

		507		0.7159

		506		0.7158

		505		0.7157

		504		0.7156

		503		0.7155

		502		0.7153

		501		0.7152

		500		0.715

		499		0.7147

		498		0.7145

		497		0.7143

		496		0.714

		495		0.7138

		494		0.7136

		493		0.7133

		492		0.7131

		491		0.7129

		490		0.7127

		489		0.7126

		488		0.7125

		487		0.7124

		486		0.7123

		485		0.7123

		484		0.7123

		483		0.7123

		482		0.7124

		481		0.7126

		480		0.7127

		479		0.7129

		478		0.7132

		477		0.7134

		476		0.7137

		475		0.7139

		474		0.7142

		473		0.7145

		472		0.7147

		471		0.715

		470		0.7152

		469		0.7154

		468		0.7156

		467		0.7158

		466		0.7159

		465		0.716

		464		0.7161

		463		0.7162

		462		0.7162

		461		0.7162

		460		0.7162

		459		0.7162

		458		0.7162

		457		0.7162

		456		0.7162

		455		0.7161

		454		0.716

		453		0.716

		452		0.7159

		451		0.7159

		450		0.7158

		449		0.7158

		448		0.7157

		447		0.7156

		446		0.7156

		445		0.7155

		444		0.7155

		443		0.7155

		442		0.7154

		441		0.7154

		440		0.7153

		439		0.7153

		438		0.7153

		437		0.7152

		436		0.7152

		435		0.7151

		434		0.7151

		433		0.7151

		432		0.715

		431		0.715

		430		0.7149

		429		0.7149

		428		0.7148

		427		0.7147

		426		0.7146

		425		0.7146

		424		0.7145

		423		0.7144

		422		0.7143

		421		0.7142

		420		0.7141

		419		0.714

		418		0.7139

		417		0.7137

		416		0.7136

		415		0.7135

		414		0.7133

		413		0.7132

		412		0.713

		411		0.7129

		410		0.7127

		409		0.7126

		408		0.7125

		407		0.7123

		406		0.7122

		405		0.712

		404		0.7118

		403		0.7117

		402		0.7115

		401		0.7113

		400		0.7112

		399		0.711

		398		0.7108

		397		0.7106

		396		0.7104

		395		0.7102

		394		0.7099

		393		0.7096

		392		0.7093

		391		0.7091

		390		0.7088

		389		0.7085

		388		0.7082

		387		0.7079

		386		0.7076

		385		0.7073

		384		0.7069

		383		0.7065

		382		0.7062

		381		0.7057

		380		0.7053

		379		0.7049

		378		0.7045

		377		0.7041

		376		0.7037

		375		0.7032

		374		0.7026

		373		0.702

		372		0.7015

		371		0.7008

		370		0.7

		369		0.6992

		368		0.6984

		367		0.6976

		366		0.6967

		365		0.6958

		364		0.695

		363		0.6941

		362		0.6932

		361		0.6923

		360		0.6913

		359		0.6904

		358		0.6894

		357		0.6884

		356		0.6873

		355		0.6864

		354		0.6855

		353		0.6847

		352		0.6839

		351		0.6831

		350		0.6822

		349		0.6814

		348		0.6806

		347		0.6798

		346		0.6789

		345		0.678

		344		0.6771

		343		0.6764

		342		0.6757

		341		0.6751

		340		0.6747

		339		0.6743

		338		0.6738

		337		0.6733

		336		0.6728

		335		0.6725

		334		0.6722

		333		0.6721

		332		0.672

		331		0.672

		330		0.672

		329		0.6722

		328		0.6724

		327		0.6726

		326		0.6728

		325		0.6729

		324		0.673

		323		0.673

		322		0.673

		321		0.6731

		320		0.6733

		319		0.6734

		318		0.6735

		317		0.6736

		316		0.6735

		315		0.6735

		314		0.6733

		313		0.6732

		312		0.6729

		311		0.6727

		310		0.6723

		309		0.672

		308		0.6717

		307		0.6713

		306		0.6709

		305		0.6704

		304		0.6699

		303		0.6693

		302		0.6687

		301		0.668

		300		0.6673

		299		0.6665

		298		0.6657

		297		0.6649

		296		0.664

		295		0.6631

		294		0.6622

		293		0.6613

		292		0.6603

		291		0.6593

		290		0.6582

		289		0.6572

		288		0.6561

		287		0.655

		286		0.6539

		285		0.6528

		284		0.6516

		283		0.6505

		282		0.6493

		281		0.6482

		280		0.647

		279		0.6458

		278		0.6446

		277		0.6434

		276		0.6421

		275		0.6408

		274		0.6396

		273		0.6382

		272		0.6369

		271		0.6356

		270		0.6342

		269		0.6328

		268		0.6313

		267		0.6298

		266		0.6283

		265		0.6267

		264		0.6251

		263		0.6234

		262		0.6217

		261		0.62

		260		0.6182

		259		0.6164

		258		0.6146

		257		0.6127

		256		0.6109

		255		0.6089

		254		0.607

		253		0.6051

		252		0.6031

		251		0.6011

		250		0.5991
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		nm		A

		1400		0.6473

		1399		0.6473

		1398		0.6474

		1397		0.6474

		1396		0.6474

		1395		0.6474

		1394		0.6474

		1393		0.6474

		1392		0.6474

		1391		0.6474

		1390		0.6475

		1389		0.6475

		1388		0.6475

		1387		0.6475

		1386		0.6476

		1385		0.6476

		1384		0.6476

		1383		0.6477

		1382		0.6477

		1381		0.6478

		1380		0.6479

		1379		0.648

		1378		0.6481

		1377		0.6482

		1376		0.6484

		1375		0.6485

		1374		0.6486

		1373		0.6487

		1372		0.6489

		1371		0.649

		1370		0.6491

		1369		0.6492

		1368		0.6493

		1367		0.6494

		1366		0.6495

		1365		0.6496

		1364		0.6497

		1363		0.6497

		1362		0.6498

		1361		0.6498

		1360		0.6498

		1359		0.6499

		1358		0.65

		1357		0.6501

		1356		0.6502

		1355		0.6503

		1354		0.6504

		1353		0.6505

		1352		0.6507

		1351		0.6508

		1350		0.651

		1349		0.6512

		1348		0.6514

		1347		0.6516

		1346		0.6518

		1345		0.652

		1344		0.6522

		1343		0.6524

		1342		0.6526

		1341		0.6528

		1340		0.653

		1339		0.6532

		1338		0.6533

		1337		0.6535

		1336		0.6537

		1335		0.6538

		1334		0.6539

		1333		0.6541

		1332		0.6542

		1331		0.6543

		1330		0.6544

		1329		0.6545

		1328		0.6546

		1327		0.6547

		1326		0.6548

		1325		0.6549

		1324		0.655

		1323		0.6551

		1322		0.6552

		1321		0.6552

		1320		0.6553

		1319		0.6554

		1318		0.6554

		1317		0.6555

		1316		0.6555

		1315		0.6556

		1314		0.6556

		1313		0.6557

		1312		0.6557

		1311		0.6557

		1310		0.6558

		1309		0.6558

		1308		0.6558

		1307		0.6559

		1306		0.6559

		1305		0.6559

		1304		0.656

		1303		0.656

		1302		0.656

		1301		0.6561

		1300		0.6562

		1299		0.6562

		1298		0.6563

		1297		0.6563

		1296		0.6564

		1295		0.6565

		1294		0.6565

		1293		0.6566

		1292		0.6567

		1291		0.6568

		1290		0.6569

		1289		0.6569

		1288		0.657

		1287		0.6571

		1286		0.6572

		1285		0.6573

		1284		0.6574

		1283		0.6575

		1282		0.6576

		1281		0.6577

		1280		0.6578

		1279		0.6579

		1278		0.658

		1277		0.6581

		1276		0.6582

		1275		0.6583

		1274		0.6584

		1273		0.6584

		1272		0.6585

		1271		0.6586

		1270		0.6586

		1269		0.6587

		1268		0.6587

		1267		0.6588

		1266		0.6588

		1265		0.6589

		1264		0.6589

		1263		0.6589

		1262		0.659

		1261		0.659

		1260		0.659

		1259		0.6591

		1258		0.6591

		1257		0.6591

		1256		0.6592

		1255		0.6593

		1254		0.6593

		1253		0.6594

		1252		0.6595

		1251		0.6596

		1250		0.6597

		1249		0.6598

		1248		0.6599

		1247		0.6601

		1246		0.6602

		1245		0.6603

		1244		0.6605

		1243		0.6606

		1242		0.6608

		1241		0.661

		1240		0.6611

		1239		0.6613

		1238		0.6615

		1237		0.6616

		1236		0.6618

		1235		0.662

		1234		0.6622

		1233		0.6624

		1232		0.6627

		1231		0.6629

		1230		0.6631

		1229		0.6634

		1228		0.6637

		1227		0.6639

		1226		0.6642

		1225		0.6644

		1224		0.6647

		1223		0.665

		1222		0.6652

		1221		0.6655

		1220		0.6657

		1219		0.6659

		1218		0.6661

		1217		0.6663

		1216		0.6665

		1215		0.6666

		1214		0.6667

		1213		0.6668

		1212		0.6669

		1211		0.6669

		1210		0.6669

		1209		0.6669

		1208		0.6669

		1207		0.6669

		1206		0.6669

		1205		0.6668

		1204		0.6667

		1203		0.6666

		1202		0.6666

		1201		0.6665

		1200		0.6664

		1199		0.6663

		1198		0.6662

		1197		0.6661

		1196		0.666

		1195		0.6659

		1194		0.6657

		1193		0.6657

		1192		0.6656

		1191		0.6655

		1190		0.6654

		1189		0.6653

		1188		0.6652

		1187		0.6651

		1186		0.665

		1185		0.6649

		1184		0.6648

		1183		0.6647

		1182		0.6646

		1181		0.6646

		1180		0.6645

		1179		0.6644

		1178		0.6644

		1177		0.6643

		1176		0.6643

		1175		0.6642

		1174		0.6642

		1173		0.6641

		1172		0.6641

		1171		0.6641

		1170		0.664

		1169		0.664

		1168		0.664

		1167		0.664

		1166		0.6639

		1165		0.6639

		1164		0.6639

		1163		0.6639

		1162		0.6639

		1161		0.6639

		1160		0.6638

		1159		0.6638

		1158		0.6638

		1157		0.6638

		1156		0.6637

		1155		0.6637

		1154		0.6637

		1153		0.6637

		1152		0.6637

		1151		0.6637

		1150		0.6637

		1149		0.6637

		1148		0.6637

		1147		0.6637

		1146		0.6637

		1145		0.6637

		1144		0.6638

		1143		0.6638

		1142		0.6638

		1141		0.6638

		1140		0.6639

		1139		0.6639

		1138		0.6639

		1137		0.6639

		1136		0.6639

		1135		0.6639

		1134		0.6639

		1133		0.6639

		1132		0.6639

		1131		0.6639

		1130		0.6639

		1129		0.6639

		1128		0.6639

		1127		0.6639

		1126		0.6638

		1125		0.6638

		1124		0.6638

		1123		0.6638

		1122		0.6638

		1121		0.6638

		1120		0.6639

		1119		0.6639

		1118		0.6639

		1117		0.6639

		1116		0.664

		1115		0.664

		1114		0.6641

		1113		0.6641

		1112		0.6642

		1111		0.6642

		1110		0.6643

		1109		0.6643

		1108		0.6644

		1107		0.6644

		1106		0.6645

		1105		0.6646

		1104		0.6646

		1103		0.6647

		1102		0.6648

		1101		0.6648

		1100		0.6649

		1099		0.6649

		1098		0.665

		1097		0.665

		1096		0.6651

		1095		0.6651

		1094		0.6651

		1093		0.6652

		1092		0.6652

		1091		0.6653

		1090		0.6653

		1089		0.6654

		1088		0.6654

		1087		0.6654

		1086		0.6655

		1085		0.6655

		1084		0.6655

		1083		0.6655

		1082		0.6656

		1081		0.6656

		1080		0.6656

		1079		0.6657

		1078		0.6657

		1077		0.6658

		1076		0.6658

		1075		0.6658

		1074		0.6658

		1073		0.6659

		1072		0.6659

		1071		0.6659

		1070		0.666

		1069		0.666

		1068		0.6661

		1067		0.6661

		1066		0.6661

		1065		0.6661

		1064		0.6661

		1063		0.6662

		1062		0.6662

		1061		0.6662

		1060		0.6662

		1059		0.6662

		1058		0.6662

		1057		0.6662

		1056		0.6662

		1055		0.6662

		1054		0.6662

		1053		0.6662

		1052		0.6662

		1051		0.6662

		1050		0.6663

		1049		0.6663

		1048		0.6663

		1047		0.6663

		1046		0.6663

		1045		0.6663

		1044		0.6663

		1043		0.6663

		1042		0.6663

		1041		0.6663

		1040		0.6663

		1039		0.6663

		1038		0.6664

		1037		0.6664

		1036		0.6664

		1035		0.6664

		1034		0.6663

		1033		0.6663

		1032		0.6663

		1031		0.6662

		1030		0.6662

		1029		0.6662

		1028		0.6662

		1027		0.6661

		1026		0.6661

		1025		0.666

		1024		0.666

		1023		0.6659

		1022		0.6659

		1021		0.6658

		1020		0.6658

		1019		0.6657

		1018		0.6657

		1017		0.6656

		1016		0.6656

		1015		0.6655

		1014		0.6655

		1013		0.6654

		1012		0.6653

		1011		0.6652

		1010		0.6652

		1009		0.6651

		1008		0.665

		1007		0.6649

		1006		0.6648

		1005		0.6647

		1004		0.6646

		1003		0.6645

		1002		0.6644

		1001		0.6642

		1000		0.6641

		999		0.664

		998		0.6638

		997		0.6636

		996		0.6635

		995		0.6633

		994		0.6631

		993		0.6629

		992		0.6628

		991		0.6626

		990		0.6624

		989		0.6621

		988		0.6619

		987		0.6617

		986		0.6615

		985		0.6612

		984		0.661

		983		0.6607

		982		0.6605

		981		0.6602

		980		0.66

		979		0.6597

		978		0.6594

		977		0.6591

		976		0.6589

		975		0.6586

		974		0.6583

		973		0.658

		972		0.6578

		971		0.6575

		970		0.6572

		969		0.6569

		968		0.6567

		967		0.6564

		966		0.6561

		965		0.6558

		964		0.6556

		963		0.6553

		962		0.655

		961		0.6548

		960		0.6545

		959		0.6542

		958		0.654

		957		0.6537

		956		0.6535

		955		0.6532

		954		0.653

		953		0.6527

		952		0.6525

		951		0.6523

		950		0.6521

		949		0.6519

		948		0.6517

		947		0.6516

		946		0.6514

		945		0.6513

		944		0.6512

		943		0.6511

		942		0.6511

		941		0.651

		940		0.651

		939		0.651

		938		0.6511

		937		0.6511

		936		0.6512

		935		0.6513

		934		0.6513

		933		0.6514

		932		0.6515

		931		0.6516

		930		0.6517

		929		0.6518

		928		0.652

		927		0.6521

		926		0.6522

		925		0.6523

		924		0.6524

		923		0.6526

		922		0.6527

		921		0.6528

		920		0.6529

		919		0.653

		918		0.6532

		917		0.6533

		916		0.6534

		915		0.6535

		914		0.6536

		913		0.6537

		912		0.6538

		911		0.6539

		910		0.654

		909		0.6541

		908		0.6542

		907		0.6543

		906		0.6544

		905		0.6544

		904		0.6545

		903		0.6546

		902		0.6548

		901		0.6549

		900		0.655

		899		0.6551

		898		0.6552

		897		0.6553

		896		0.6555

		895		0.6556

		894		0.6558

		893		0.6559

		892		0.6561

		891		0.6562

		890		0.6564

		889		0.6565

		888		0.6567

		887		0.6568

		886		0.6569

		885		0.6569

		884		0.657

		883		0.6571

		882		0.6572

		881		0.6572

		880		0.6573

		879		0.6574

		878		0.6574

		877		0.6575

		876		0.6576

		875		0.6577

		874		0.6579

		873		0.6581

		872		0.6584

		871		0.6588

		870		0.6592

		869		0.6597

		868		0.6603

		867		0.6609

		866		0.6615

		865		0.6622

		864		0.663

		863		0.6638

		862		0.6647

		861		0.6656

		860		0.6666

		859		0.6675

		858		0.6684

		857		0.6694

		856		0.6702

		855		0.671

		854		0.6718

		853		0.6725

		852		0.6731

		851		0.6737

		850		0.6741

		849		0.6746

		848		0.6749

		847		0.6753

		846		0.6755

		845		0.6757

		844		0.6758

		843		0.6759

		842		0.676

		841		0.6759

		840		0.6759

		839		0.6758

		838		0.6758

		837		0.6757

		836		0.6756

		835		0.6755

		834		0.6754

		833		0.6754

		832		0.6753

		831		0.6753

		830		0.6752

		829		0.6751

		828		0.675

		827		0.6749

		826		0.6748

		825		0.6747

		824		0.6747

		823		0.6746

		822		0.6746

		821		0.6746

		820		0.6746

		819		0.6746

		818		0.6746

		817		0.6746

		816		0.6745

		815		0.6745

		814		0.6745

		813		0.6746

		812		0.6746

		811		0.6747

		810		0.6747

		809		0.6748

		808		0.6749

		807		0.675

		806		0.6751

		805		0.6751

		804		0.6752

		803		0.6753

		802		0.6754

		801		0.6755

		800		0.6755

		799		0.6756

		798		0.6757

		797		0.6758

		796		0.6758

		795		0.6759

		794		0.6759

		793		0.6759

		792		0.6759

		791		0.676

		790		0.676

		789		0.676

		788		0.676

		787		0.676

		786		0.676

		785		0.6761

		784		0.6761

		783		0.6761

		782		0.6761

		781		0.6761

		780		0.6761

		779		0.6762

		778		0.6762

		777		0.6763

		776		0.6763

		775		0.6764

		774		0.6765

		773		0.6766

		772		0.6766

		771		0.6767

		770		0.6768

		769		0.6769

		768		0.6769

		767		0.677

		766		0.6771

		765		0.6772

		764		0.6773

		763		0.6773

		762		0.6774

		761		0.6774

		760		0.6774

		759		0.6774

		758		0.6774

		757		0.6774

		756		0.6774

		755		0.6774

		754		0.6774

		753		0.6775

		752		0.6775

		751		0.6775

		750		0.6775

		749		0.6775

		748		0.6775

		747		0.6775

		746		0.6775

		745		0.6776

		744		0.6776

		743		0.6777

		742		0.6778

		741		0.6778

		740		0.6779

		739		0.6779

		738		0.678

		737		0.678

		736		0.678

		735		0.6781

		734		0.6781

		733		0.6782

		732		0.6782

		731		0.6783

		730		0.6783

		729		0.6783

		728		0.6784

		727		0.6784

		726		0.6784

		725		0.6784

		724		0.6785

		723		0.6785

		722		0.6785

		721		0.6786

		720		0.6786

		719		0.6787

		718		0.6787

		717		0.6787

		716		0.6788

		715		0.6788

		714		0.6788

		713		0.6788

		712		0.6789

		711		0.6789

		710		0.6789

		709		0.679

		708		0.679

		707		0.679

		706		0.6791

		705		0.6791

		704		0.6791

		703		0.6792

		702		0.6792

		701		0.6793

		700		0.6793

		699		0.6794

		698		0.6794

		697		0.6794

		696		0.6795

		695		0.6795

		694		0.6795

		693		0.6796

		692		0.6796

		691		0.6796

		690		0.6797

		689		0.6797

		688		0.6797

		687		0.6798

		686		0.6798

		685		0.6798

		684		0.6798

		683		0.6799

		682		0.6799

		681		0.6799

		680		0.68

		679		0.68

		678		0.6801

		677		0.6801

		676		0.6802

		675		0.6802

		674		0.6803

		673		0.6803

		672		0.6804

		671		0.6804

		670		0.6804

		669		0.6804

		668		0.6805

		667		0.6805

		666		0.6805

		665		0.6805

		664		0.6806

		663		0.6806

		662		0.6806

		661		0.6806

		660		0.6807

		659		0.6807

		658		0.6807

		657		0.6808

		656		0.6808

		655		0.6809

		654		0.6809

		653		0.681

		652		0.681

		651		0.6811

		650		0.6811

		649		0.6812

		648		0.6812

		647		0.6813

		646		0.6813

		645		0.6813

		644		0.6814

		643		0.6814

		642		0.6814

		641		0.6814

		640		0.6815

		639		0.6815

		638		0.6815

		637		0.6815

		636		0.6815

		635		0.6816

		634		0.6816

		633		0.6816

		632		0.6816

		631		0.6816

		630		0.6817

		629		0.6817

		628		0.6817

		627		0.6818

		626		0.6818

		625		0.6818

		624		0.6819

		623		0.6819

		622		0.682

		621		0.682

		620		0.682

		619		0.6821

		618		0.6821

		617		0.6822

		616		0.6822

		615		0.6822

		614		0.6823

		613		0.6823

		612		0.6823

		611		0.6823

		610		0.6824

		609		0.6824

		608		0.6824

		607		0.6824

		606		0.6824

		605		0.6824

		604		0.6824

		603		0.6825

		602		0.6825

		601		0.6825

		600		0.6825

		599		0.6825

		598		0.6826

		597		0.6826

		596		0.6826

		595		0.6826

		594		0.6827

		593		0.6827

		592		0.6827

		591		0.6828

		590		0.6828

		589		0.6828

		588		0.6829

		587		0.6829

		586		0.6829

		585		0.6829

		584		0.6829

		583		0.6829

		582		0.6829

		581		0.683

		580		0.683

		579		0.6829

		578		0.6829

		577		0.6829

		576		0.6829

		575		0.6828

		574		0.6828

		573		0.6828

		572		0.6827

		571		0.6826

		570		0.6826

		569		0.6825

		568		0.6824

		567		0.6824

		566		0.6823

		565		0.6822

		564		0.6821

		563		0.682

		562		0.682

		561		0.6819

		560		0.6818

		559		0.6817

		558		0.6817

		557		0.6816

		556		0.6816

		555		0.6816

		554		0.6816

		553		0.6815

		552		0.6815

		551		0.6816

		550		0.6816

		549		0.6816

		548		0.6817

		547		0.6818

		546		0.6819

		545		0.682

		544		0.6821

		543		0.6822

		542		0.6824

		541		0.6825

		540		0.6827

		539		0.6829

		538		0.6832

		537		0.6834

		536		0.6837

		535		0.684

		534		0.6843

		533		0.6847

		532		0.685

		531		0.6854

		530		0.6858

		529		0.6862

		528		0.6867

		527		0.6871

		526		0.6876

		525		0.6881

		524		0.6885

		523		0.689

		522		0.6895

		521		0.69

		520		0.6904

		519		0.6908

		518		0.6912

		517		0.6916

		516		0.692

		515		0.6923

		514		0.6925

		513		0.6928

		512		0.6929

		511		0.6931

		510		0.6931

		509		0.6932

		508		0.6931

		507		0.6931

		506		0.6929

		505		0.6928

		504		0.6926

		503		0.6924

		502		0.6921

		501		0.6918

		500		0.6915

		499		0.6912

		498		0.6909

		497		0.6905

		496		0.6902

		495		0.6898

		494		0.6895

		493		0.6892

		492		0.6889

		491		0.6886

		490		0.6884

		489		0.6882

		488		0.688

		487		0.6879

		486		0.6878

		485		0.6878

		484		0.6878

		483		0.6879

		482		0.6881

		481		0.6883

		480		0.6885

		479		0.6888

		478		0.6891

		477		0.6894

		476		0.6897

		475		0.6901

		474		0.6904

		473		0.6908

		472		0.6911

		471		0.6915

		470		0.6917

		469		0.692

		468		0.6923

		467		0.6925

		466		0.6926

		465		0.6927

		464		0.6928

		463		0.6929

		462		0.6929

		461		0.6929

		460		0.6929

		459		0.6928

		458		0.6928

		457		0.6927

		456		0.6926

		455		0.6925

		454		0.6923

		453		0.6922

		452		0.6921

		451		0.692

		450		0.6919

		449		0.6918

		448		0.6917

		447		0.6916

		446		0.6915

		445		0.6915

		444		0.6914

		443		0.6913

		442		0.6913

		441		0.6912

		440		0.6912

		439		0.6912

		438		0.6911

		437		0.6911

		436		0.6911

		435		0.6911

		434		0.6911

		433		0.6911

		432		0.6911

		431		0.6911

		430		0.691

		429		0.691

		428		0.691

		427		0.6909

		426		0.6909

		425		0.6908

		424		0.6908

		423		0.6907

		422		0.6906

		421		0.6906

		420		0.6904

		419		0.6903

		418		0.6902

		417		0.6901

		416		0.6899

		415		0.6898

		414		0.6896

		413		0.6894

		412		0.6893

		411		0.6891

		410		0.6889

		409		0.6888

		408		0.6886

		407		0.6884

		406		0.6882

		405		0.688

		404		0.6879

		403		0.6877

		402		0.6875

		401		0.6873

		400		0.6871

		399		0.687

		398		0.6868

		397		0.6866

		396		0.6864

		395		0.6861

		394		0.6859

		393		0.6855

		392		0.6851

		391		0.6847

		390		0.6843

		389		0.6839

		388		0.6834

		387		0.683

		386		0.6824

		385		0.6818

		384		0.6811

		383		0.6804

		382		0.6797

		381		0.6788

		380		0.678

		379		0.6771

		378		0.6762

		377		0.6754

		376		0.6747

		375		0.6741

		374		0.6733

		373		0.6726

		372		0.6717

		371		0.6709

		370		0.6701

		369		0.6694

		368		0.6688

		367		0.6682

		366		0.6677

		365		0.6673

		364		0.6668

		363		0.6663

		362		0.6658

		361		0.6652

		360		0.6645

		359		0.6638

		358		0.6631

		357		0.6624

		356		0.6618

		355		0.6613

		354		0.6607

		353		0.6602

		352		0.6596

		351		0.659

		350		0.6583

		349		0.6577

		348		0.6571

		347		0.6565

		346		0.656

		345		0.6556

		344		0.6553

		343		0.655

		342		0.6547

		341		0.6544

		340		0.6543

		339		0.6541

		338		0.6537

		337		0.6533

		336		0.6528

		335		0.6523

		334		0.6518

		333		0.6513

		332		0.6508

		331		0.6505

		330		0.6503

		329		0.6501

		328		0.6498

		327		0.6495

		326		0.6493

		325		0.649

		324		0.6488

		323		0.6487

		322		0.6486

		321		0.6488

		320		0.6492

		319		0.6497

		318		0.6503

		317		0.6509

		316		0.6515

		315		0.652

		314		0.6524

		313		0.6527

		312		0.6529

		311		0.6532

		310		0.6533

		309		0.6535

		308		0.6536

		307		0.6536

		306		0.6535

		305		0.6533

		304		0.653

		303		0.6525

		302		0.6519

		301		0.6512

		300		0.6505

		299		0.6497

		298		0.6489

		297		0.6481

		296		0.6472

		295		0.6463

		294		0.6454

		293		0.6444

		292		0.6434

		291		0.6424

		290		0.6414

		289		0.6403

		288		0.6392

		287		0.6381

		286		0.6369

		285		0.6358

		284		0.6347

		283		0.6335

		282		0.6323

		281		0.6311

		280		0.6299

		279		0.6287

		278		0.6274

		277		0.6262

		276		0.6249

		275		0.6236

		274		0.6223

		273		0.6209

		272		0.6196

		271		0.6181

		270		0.6167

		269		0.6152

		268		0.6137

		267		0.6121

		266		0.6105

		265		0.6089

		264		0.6072

		263		0.6055

		262		0.6037

		261		0.602

		260		0.6001

		259		0.5983

		258		0.5965

		257		0.5946

		256		0.5927

		255		0.5908

		254		0.5889

		253		0.587

		252		0.585

		251		0.5831

		250		0.5811
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		nm		A

		1400		0.6155

		1399		0.6156

		1398		0.6157

		1397		0.6159

		1396		0.616

		1395		0.6161

		1394		0.6161

		1393		0.6162

		1392		0.6163

		1391		0.6163

		1390		0.6163

		1389		0.6163

		1388		0.6163

		1387		0.6163

		1386		0.6162

		1385		0.6162

		1384		0.6161

		1383		0.6161

		1382		0.616

		1381		0.616

		1380		0.616

		1379		0.6159

		1378		0.6159

		1377		0.6159

		1376		0.6159

		1375		0.616

		1374		0.616

		1373		0.616

		1372		0.6161

		1371		0.6162

		1370		0.6162

		1369		0.6163

		1368		0.6164

		1367		0.6164

		1366		0.6165

		1365		0.6165

		1364		0.6166

		1363		0.6166

		1362		0.6166

		1361		0.6166

		1360		0.6166

		1359		0.6166

		1358		0.6166

		1357		0.6165

		1356		0.6165

		1355		0.6165

		1354		0.6165

		1353		0.6165

		1352		0.6164

		1351		0.6164

		1350		0.6164

		1349		0.6164

		1348		0.6164

		1347		0.6165

		1346		0.6165

		1345		0.6165

		1344		0.6166

		1343		0.6166

		1342		0.6167

		1341		0.6167

		1340		0.6168

		1339		0.6169

		1338		0.6169

		1337		0.617

		1336		0.6171

		1335		0.6172

		1334		0.6173

		1333		0.6174

		1332		0.6175

		1331		0.6175

		1330		0.6176

		1329		0.6177

		1328		0.6178

		1327		0.6179

		1326		0.618

		1325		0.6181

		1324		0.6182

		1323		0.6183

		1322		0.6184

		1321		0.6185

		1320		0.6186

		1319		0.6187

		1318		0.6188

		1317		0.6189

		1316		0.619

		1315		0.619

		1314		0.6191

		1313		0.6192

		1312		0.6193

		1311		0.6194

		1310		0.6195

		1309		0.6196

		1308		0.6197

		1307		0.6198

		1306		0.6199

		1305		0.62

		1304		0.6201

		1303		0.6202

		1302		0.6202

		1301		0.6203

		1300		0.6204

		1299		0.6205

		1298		0.6206

		1297		0.6206

		1296		0.6207

		1295		0.6208

		1294		0.6208

		1293		0.6209

		1292		0.621

		1291		0.621

		1290		0.6211

		1289		0.6211

		1288		0.6212

		1287		0.6212

		1286		0.6213

		1285		0.6213

		1284		0.6214

		1283		0.6214

		1282		0.6215

		1281		0.6215

		1280		0.6216

		1279		0.6216

		1278		0.6216

		1277		0.6217

		1276		0.6217

		1275		0.6218

		1274		0.6218

		1273		0.6219

		1272		0.622

		1271		0.6221

		1270		0.6222

		1269		0.6223

		1268		0.6224

		1267		0.6225

		1266		0.6226

		1265		0.6228

		1264		0.6229

		1263		0.623

		1262		0.6231

		1261		0.6233

		1260		0.6234

		1259		0.6236

		1258		0.6237

		1257		0.6239

		1256		0.624

		1255		0.6242

		1254		0.6243

		1253		0.6244

		1252		0.6245

		1251		0.6246

		1250		0.6248

		1249		0.6249

		1248		0.625

		1247		0.6252

		1246		0.6253

		1245		0.6255

		1244		0.6257

		1243		0.6259

		1242		0.6261

		1241		0.6263

		1240		0.6265

		1239		0.6268

		1238		0.6271

		1237		0.6274

		1236		0.6277

		1235		0.6281

		1234		0.6285

		1233		0.6289

		1232		0.6293

		1231		0.6298

		1230		0.6302

		1229		0.6307

		1228		0.6311

		1227		0.6316

		1226		0.6321

		1225		0.6326

		1224		0.6331

		1223		0.6336

		1222		0.634

		1221		0.6344

		1220		0.6348

		1219		0.6352

		1218		0.6355

		1217		0.6358

		1216		0.6361

		1215		0.6363

		1214		0.6364

		1213		0.6366

		1212		0.6367

		1211		0.6367

		1210		0.6367

		1209		0.6367

		1208		0.6367

		1207		0.6366

		1206		0.6365

		1205		0.6363

		1204		0.6362

		1203		0.636

		1202		0.6359

		1201		0.6357

		1200		0.6356

		1199		0.6354

		1198		0.6352

		1197		0.6351

		1196		0.6349

		1195		0.6348

		1194		0.6346

		1193		0.6344

		1192		0.6343

		1191		0.6341

		1190		0.634

		1189		0.6339

		1188		0.6337

		1187		0.6336

		1186		0.6334

		1185		0.6333

		1184		0.6331

		1183		0.633

		1182		0.6329

		1181		0.6327

		1180		0.6326

		1179		0.6325

		1178		0.6324

		1177		0.6323

		1176		0.6322

		1175		0.6321

		1174		0.632

		1173		0.632

		1172		0.6319

		1171		0.6318

		1170		0.6318

		1169		0.6317

		1168		0.6316

		1167		0.6316

		1166		0.6315

		1165		0.6315

		1164		0.6315

		1163		0.6314

		1162		0.6314

		1161		0.6313

		1160		0.6313

		1159		0.6312

		1158		0.6312

		1157		0.6311

		1156		0.6311

		1155		0.631

		1154		0.631

		1153		0.631

		1152		0.6309

		1151		0.6309

		1150		0.6309

		1149		0.6309

		1148		0.6309

		1147		0.6309

		1146		0.6309

		1145		0.6309

		1144		0.6309

		1143		0.6309

		1142		0.6309

		1141		0.6309

		1140		0.631

		1139		0.631

		1138		0.6311

		1137		0.6311

		1136		0.6311

		1135		0.6312

		1134		0.6312

		1133		0.6313

		1132		0.6313

		1131		0.6314

		1130		0.6314

		1129		0.6315

		1128		0.6315

		1127		0.6316

		1126		0.6316

		1125		0.6317

		1124		0.6318

		1123		0.6318

		1122		0.6319

		1121		0.632

		1120		0.632

		1119		0.6321

		1118		0.6322

		1117		0.6322

		1116		0.6323

		1115		0.6324

		1114		0.6325

		1113		0.6326

		1112		0.6326

		1111		0.6327

		1110		0.6328

		1109		0.6329

		1108		0.633

		1107		0.6331

		1106		0.6332

		1105		0.6332

		1104		0.6333

		1103		0.6334

		1102		0.6335

		1101		0.6336

		1100		0.6337

		1099		0.6338

		1098		0.6339

		1097		0.6339

		1096		0.634

		1095		0.6341

		1094		0.6342

		1093		0.6343

		1092		0.6344

		1091		0.6344

		1090		0.6345

		1089		0.6346

		1088		0.6347

		1087		0.6347

		1086		0.6348

		1085		0.6349

		1084		0.6349

		1083		0.635

		1082		0.6351

		1081		0.6352

		1080		0.6352

		1079		0.6353

		1078		0.6354

		1077		0.6355

		1076		0.6356

		1075		0.6356

		1074		0.6357

		1073		0.6358

		1072		0.6359

		1071		0.636

		1070		0.636

		1069		0.6361

		1068		0.6362

		1067		0.6363

		1066		0.6364

		1065		0.6365

		1064		0.6366

		1063		0.6367

		1062		0.6367

		1061		0.6368

		1060		0.6369

		1059		0.637

		1058		0.6371

		1057		0.6372

		1056		0.6373

		1055		0.6374

		1054		0.6375

		1053		0.6376

		1052		0.6377

		1051		0.6378

		1050		0.6379

		1049		0.638

		1048		0.6381

		1047		0.6382

		1046		0.6383

		1045		0.6384

		1044		0.6384

		1043		0.6385

		1042		0.6386

		1041		0.6387

		1040		0.6387

		1039		0.6388

		1038		0.6388

		1037		0.6388

		1036		0.6389

		1035		0.6389

		1034		0.6389

		1033		0.6389

		1032		0.6389

		1031		0.639

		1030		0.639

		1029		0.639

		1028		0.639

		1027		0.639

		1026		0.639

		1025		0.639

		1024		0.6391

		1023		0.6391

		1022		0.6391

		1021		0.6391

		1020		0.6391

		1019		0.6391

		1018		0.6391

		1017		0.6391

		1016		0.6391

		1015		0.6391

		1014		0.6391

		1013		0.6391

		1012		0.6391

		1011		0.6391

		1010		0.639

		1009		0.639

		1008		0.639

		1007		0.6389

		1006		0.6389

		1005		0.6388

		1004		0.6388

		1003		0.6387

		1002		0.6386

		1001		0.6385

		1000		0.6384

		999		0.6383

		998		0.6382

		997		0.6381

		996		0.638

		995		0.6379

		994		0.6378

		993		0.6376

		992		0.6375

		991		0.6373

		990		0.6372

		989		0.637

		988		0.6368

		987		0.6366

		986		0.6364

		985		0.6362

		984		0.636

		983		0.6358

		982		0.6356

		981		0.6354

		980		0.6351

		979		0.6349

		978		0.6346

		977		0.6344

		976		0.6341

		975		0.6339

		974		0.6336

		973		0.6334

		972		0.6331

		971		0.6328

		970		0.6326

		969		0.6323

		968		0.632

		967		0.6318

		966		0.6315

		965		0.6312

		964		0.6309

		963		0.6307

		962		0.6304

		961		0.6302

		960		0.6299

		959		0.6296

		958		0.6294

		957		0.6291

		956		0.6289

		955		0.6286

		954		0.6284

		953		0.6282

		952		0.628

		951		0.6278

		950		0.6277

		949		0.6275

		948		0.6274

		947		0.6273

		946		0.6272

		945		0.6271

		944		0.627

		943		0.627

		942		0.627

		941		0.627

		940		0.627

		939		0.627

		938		0.627

		937		0.6271

		936		0.6272

		935		0.6272

		934		0.6273

		933		0.6274

		932		0.6275

		931		0.6276

		930		0.6277

		929		0.6278

		928		0.6279

		927		0.6281

		926		0.6282

		925		0.6283

		924		0.6284

		923		0.6285

		922		0.6286

		921		0.6288

		920		0.6289

		919		0.629

		918		0.6291

		917		0.6292

		916		0.6293

		915		0.6294

		914		0.6295

		913		0.6296

		912		0.6297

		911		0.6298

		910		0.6299

		909		0.63

		908		0.6301

		907		0.6302

		906		0.6303

		905		0.6304

		904		0.6305

		903		0.6305

		902		0.6306

		901		0.6307

		900		0.6307

		899		0.6308

		898		0.6309

		897		0.631

		896		0.6311

		895		0.6311

		894		0.6312

		893		0.6313

		892		0.6314

		891		0.6314

		890		0.6315

		889		0.6316

		888		0.6317

		887		0.6318

		886		0.6318

		885		0.6319

		884		0.632

		883		0.6321

		882		0.6323

		881		0.6323

		880		0.6324

		879		0.6325

		878		0.6326

		877		0.6326

		876		0.6327

		875		0.6329

		874		0.633

		873		0.6332

		872		0.6335

		871		0.6338

		870		0.6341

		869		0.6344

		868		0.6349

		867		0.6353

		866		0.6358

		865		0.6363

		864		0.637

		863		0.6376

		862		0.6383

		861		0.6389

		860		0.6397

		859		0.6404

		858		0.6412

		857		0.6419

		856		0.6425

		855		0.643

		854		0.6435

		853		0.644

		852		0.6443

		851		0.6447

		850		0.6449

		849		0.6452

		848		0.6453

		847		0.6455

		846		0.6455

		845		0.6456

		844		0.6455

		843		0.6454

		842		0.6453

		841		0.6451

		840		0.645

		839		0.6449

		838		0.6448

		837		0.6447

		836		0.6446

		835		0.6445

		834		0.6445

		833		0.6444

		832		0.6443

		831		0.6441

		830		0.644

		829		0.6439

		828		0.6439

		827		0.6438

		826		0.6438

		825		0.6438

		824		0.6437

		823		0.6437

		822		0.6437

		821		0.6436

		820		0.6436

		819		0.6436

		818		0.6435

		817		0.6435

		816		0.6435

		815		0.6435

		814		0.6435

		813		0.6435

		812		0.6435

		811		0.6435

		810		0.6435

		809		0.6435

		808		0.6435

		807		0.6435

		806		0.6436

		805		0.6436

		804		0.6436

		803		0.6437

		802		0.6437

		801		0.6438

		800		0.6438

		799		0.6439

		798		0.6439

		797		0.644

		796		0.6441

		795		0.6441

		794		0.6442

		793		0.6443

		792		0.6444

		791		0.6445

		790		0.6445

		789		0.6446

		788		0.6447

		787		0.6447

		786		0.6448

		785		0.6449

		784		0.6449

		783		0.645

		782		0.645

		781		0.6451

		780		0.6451

		779		0.6452

		778		0.6452

		777		0.6452

		776		0.6452

		775		0.6453

		774		0.6453

		773		0.6453

		772		0.6454

		771		0.6454

		770		0.6454

		769		0.6455

		768		0.6455

		767		0.6455

		766		0.6455

		765		0.6455

		764		0.6455

		763		0.6456

		762		0.6456

		761		0.6456

		760		0.6457

		759		0.6457

		758		0.6458

		757		0.6458

		756		0.6459

		755		0.646

		754		0.646

		753		0.6461

		752		0.6462

		751		0.6462

		750		0.6463

		749		0.6464

		748		0.6465

		747		0.6465

		746		0.6466

		745		0.6466

		744		0.6467

		743		0.6467

		742		0.6468

		741		0.6468

		740		0.6468

		739		0.6468

		738		0.6468

		737		0.6468

		736		0.6467

		735		0.6467

		734		0.6467

		733		0.6467

		732		0.6467

		731		0.6467

		730		0.6467

		729		0.6467

		728		0.6467

		727		0.6467

		726		0.6467

		725		0.6468

		724		0.6468

		723		0.6469

		722		0.647

		721		0.647

		720		0.6471

		719		0.6472

		718		0.6473

		717		0.6474

		716		0.6475

		715		0.6475

		714		0.6476

		713		0.6477

		712		0.6477

		711		0.6478

		710		0.6478

		709		0.6479

		708		0.6479

		707		0.648

		706		0.648

		705		0.648

		704		0.6481

		703		0.6481

		702		0.6481

		701		0.6482

		700		0.6482

		699		0.6482

		698		0.6482

		697		0.6483

		696		0.6483

		695		0.6483

		694		0.6483

		693		0.6484

		692		0.6484

		691		0.6484

		690		0.6485

		689		0.6485

		688		0.6485

		687		0.6486

		686		0.6486

		685		0.6486

		684		0.6487

		683		0.6487

		682		0.6487

		681		0.6488

		680		0.6488

		679		0.6489

		678		0.6489

		677		0.649

		676		0.649

		675		0.6491

		674		0.6491

		673		0.6492

		672		0.6492

		671		0.6493

		670		0.6493

		669		0.6493

		668		0.6494

		667		0.6494

		666		0.6495

		665		0.6495

		664		0.6495

		663		0.6496

		662		0.6496

		661		0.6496

		660		0.6497

		659		0.6497

		658		0.6498

		657		0.6498

		656		0.6498

		655		0.6499

		654		0.6499

		653		0.65

		652		0.65

		651		0.65

		650		0.6501

		649		0.6501

		648		0.6501

		647		0.6502

		646		0.6502

		645		0.6502

		644		0.6502

		643		0.6502

		642		0.6502

		641		0.6502

		640		0.6502

		639		0.6502

		638		0.6502

		637		0.6502

		636		0.6502

		635		0.6502

		634		0.6502

		633		0.6502

		632		0.6502

		631		0.6502

		630		0.6502

		629		0.6502

		628		0.6503

		627		0.6503

		626		0.6504

		625		0.6504

		624		0.6505

		623		0.6505

		622		0.6506

		621		0.6506

		620		0.6507

		619		0.6508

		618		0.6508

		617		0.6509

		616		0.6509

		615		0.651

		614		0.651

		613		0.651

		612		0.6511

		611		0.6511

		610		0.6511

		609		0.6511

		608		0.6511

		607		0.6511

		606		0.6511

		605		0.6511

		604		0.6511

		603		0.6511

		602		0.6511

		601		0.6511

		600		0.6511

		599		0.6511

		598		0.6511

		597		0.6512

		596		0.6512

		595		0.6512

		594		0.6512

		593		0.6512

		592		0.6512

		591		0.6512

		590		0.6512

		589		0.6513

		588		0.6513

		587		0.6513

		586		0.6513

		585		0.6513

		584		0.6513

		583		0.6513

		582		0.6513

		581		0.6513

		580		0.6513

		579		0.6512

		578		0.6512

		577		0.6512

		576		0.6511

		575		0.651

		574		0.651

		573		0.6509

		572		0.6508

		571		0.6507

		570		0.6506

		569		0.6504

		568		0.6503

		567		0.6502

		566		0.65

		565		0.6499

		564		0.6497

		563		0.6496

		562		0.6494

		561		0.6492

		560		0.6491

		559		0.649

		558		0.6489

		557		0.6488

		556		0.6487

		555		0.6487

		554		0.6486

		553		0.6486

		552		0.6486

		551		0.6486

		550		0.6486

		549		0.6487

		548		0.6487

		547		0.6488

		546		0.6489

		545		0.649

		544		0.6492

		543		0.6493

		542		0.6495

		541		0.6496

		540		0.6498

		539		0.6501

		538		0.6503

		537		0.6505

		536		0.6508

		535		0.6512

		534		0.6515

		533		0.6519

		532		0.6522

		531		0.6527

		530		0.6531

		529		0.6535

		528		0.654

		527		0.6545

		526		0.655

		525		0.6555

		524		0.656

		523		0.6565

		522		0.6569

		521		0.6574

		520		0.6579

		519		0.6583

		518		0.6587

		517		0.6591

		516		0.6594

		515		0.6597

		514		0.6599

		513		0.6601

		512		0.6602

		511		0.6603

		510		0.6604

		509		0.6604

		508		0.6603

		507		0.6602

		506		0.6601

		505		0.6599

		504		0.6597

		503		0.6595

		502		0.6592

		501		0.6589

		500		0.6586

		499		0.6583

		498		0.658

		497		0.6576

		496		0.6573

		495		0.657

		494		0.6567

		493		0.6564

		492		0.6561

		491		0.6559

		490		0.6556

		489		0.6555

		488		0.6553

		487		0.6552

		486		0.6551

		485		0.6551

		484		0.6551

		483		0.6552

		482		0.6553

		481		0.6555

		480		0.6557

		479		0.6559

		478		0.6562

		477		0.6565

		476		0.6569

		475		0.6572

		474		0.6575

		473		0.6579

		472		0.6582

		471		0.6585

		470		0.6588

		469		0.6591

		468		0.6594

		467		0.6596

		466		0.6598

		465		0.6599

		464		0.6601

		463		0.6602

		462		0.6602

		461		0.6603

		460		0.6603

		459		0.6602

		458		0.6602

		457		0.6601

		456		0.66

		455		0.6599

		454		0.6598

		453		0.6597

		452		0.6596

		451		0.6595

		450		0.6594

		449		0.6593

		448		0.6592

		447		0.6591

		446		0.659

		445		0.6589

		444		0.6588

		443		0.6588

		442		0.6587

		441		0.6587

		440		0.6587

		439		0.6587

		438		0.6587

		437		0.6587

		436		0.6587

		435		0.6587

		434		0.6587

		433		0.6587

		432		0.6587

		431		0.6587

		430		0.6586

		429		0.6586

		428		0.6586

		427		0.6585

		426		0.6585

		425		0.6584

		424		0.6584

		423		0.6583

		422		0.6583

		421		0.6582

		420		0.6581

		419		0.658

		418		0.6579

		417		0.6578

		416		0.6577

		415		0.6576

		414		0.6575

		413		0.6574

		412		0.6573

		411		0.6572

		410		0.6571

		409		0.657

		408		0.6569

		407		0.6568

		406		0.6567

		405		0.6565

		404		0.6564

		403		0.6563

		402		0.6562

		401		0.656

		400		0.6559

		399		0.6558

		398		0.6556

		397		0.6555

		396		0.6553

		395		0.6551

		394		0.6548

		393		0.6545

		392		0.6542

		391		0.6538

		390		0.6534

		389		0.653

		388		0.6525

		387		0.6519

		386		0.6513

		385		0.6506

		384		0.6499

		383		0.6491

		382		0.6482

		381		0.6473

		380		0.6463

		379		0.6453

		378		0.6442

		377		0.6433

		376		0.6423

		375		0.6414

		374		0.6404

		373		0.6395

		372		0.6386

		371		0.6376

		370		0.6367

		369		0.6358

		368		0.6351

		367		0.6343

		366		0.6336

		365		0.6329

		364		0.6323

		363		0.6317

		362		0.6313

		361		0.6308

		360		0.6303

		359		0.6298

		358		0.6292

		357		0.6286

		356		0.628

		355		0.6276

		354		0.6272

		353		0.6268

		352		0.6263

		351		0.6258

		350		0.6254

		349		0.625

		348		0.6246

		347		0.6242

		346		0.6237

		345		0.6232

		344		0.6226

		343		0.6221

		342		0.6216

		341		0.6212

		340		0.6209

		339		0.6205

		338		0.6199

		337		0.6194

		336		0.6189

		335		0.6185

		334		0.6182

		333		0.6179

		332		0.6177

		331		0.6175

		330		0.6174

		329		0.6174

		328		0.6175

		327		0.6177

		326		0.6179

		325		0.6181

		324		0.6185

		323		0.6189

		322		0.6194

		321		0.62

		320		0.6206

		319		0.6212

		318		0.6218

		317		0.6222

		316		0.6226

		315		0.623

		314		0.6233

		313		0.6235

		312		0.6236

		311		0.6236

		310		0.6236

		309		0.6235

		308		0.6233

		307		0.6229

		306		0.6225

		305		0.622

		304		0.6214

		303		0.6208

		302		0.6201

		301		0.6193

		300		0.6186

		299		0.6178

		298		0.617

		297		0.6161

		296		0.6153

		295		0.6143

		294		0.6134

		293		0.6124

		292		0.6114

		291		0.6103

		290		0.6092

		289		0.6081

		288		0.607

		287		0.6058

		286		0.6047

		285		0.6035

		284		0.6023

		283		0.6011

		282		0.5998

		281		0.5986

		280		0.5974

		279		0.5961

		278		0.5948

		277		0.5935

		276		0.5922

		275		0.5909

		274		0.5895

		273		0.5882

		272		0.5868

		271		0.5854

		270		0.5839

		269		0.5824

		268		0.5809

		267		0.5793

		266		0.5777

		265		0.576

		264		0.5743

		263		0.5725

		262		0.5708

		261		0.5689

		260		0.5671

		259		0.5652

		258		0.5633

		257		0.5614

		256		0.5595

		255		0.5575

		254		0.5556

		253		0.5536

		252		0.5516

		251		0.5496

		250		0.5476
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		nm		A

		1400		0.566

		1399		0.5662

		1398		0.5663

		1397		0.5665

		1396		0.5667

		1395		0.5668

		1394		0.567

		1393		0.5671

		1392		0.5672

		1391		0.5672

		1390		0.5673

		1389		0.5673

		1388		0.5672

		1387		0.5672

		1386		0.5672

		1385		0.5671

		1384		0.567

		1383		0.5669

		1382		0.5669

		1381		0.5668

		1380		0.5667

		1379		0.5666

		1378		0.5665

		1377		0.5664

		1376		0.5663

		1375		0.5663

		1374		0.5662

		1373		0.5662

		1372		0.5661

		1371		0.5661

		1370		0.5661

		1369		0.5661

		1368		0.5661

		1367		0.5662

		1366		0.5662

		1365		0.5662

		1364		0.5663

		1363		0.5663

		1362		0.5664

		1361		0.5665

		1360		0.5665

		1359		0.5666

		1358		0.5667

		1357		0.5668

		1356		0.5668

		1355		0.5669

		1354		0.567

		1353		0.5671

		1352		0.5672

		1351		0.5673

		1350		0.5673

		1349		0.5674

		1348		0.5675

		1347		0.5675

		1346		0.5676

		1345		0.5677

		1344		0.5678

		1343		0.5679

		1342		0.5679

		1341		0.568

		1340		0.5681

		1339		0.5682

		1338		0.5682

		1337		0.5683

		1336		0.5684

		1335		0.5684

		1334		0.5685

		1333		0.5686

		1332		0.5687

		1331		0.5687

		1330		0.5688

		1329		0.5689

		1328		0.569

		1327		0.569

		1326		0.5691

		1325		0.5692

		1324		0.5693

		1323		0.5694

		1322		0.5695

		1321		0.5695

		1320		0.5696

		1319		0.5697

		1318		0.5698

		1317		0.5699

		1316		0.5699

		1315		0.57

		1314		0.5701

		1313		0.5702

		1312		0.5702

		1311		0.5703

		1310		0.5704

		1309		0.5705

		1308		0.5705

		1307		0.5706

		1306		0.5707

		1305		0.5707

		1304		0.5708

		1303		0.5709

		1302		0.571

		1301		0.571

		1300		0.5711

		1299		0.5712

		1298		0.5713

		1297		0.5714

		1296		0.5715

		1295		0.5716

		1294		0.5717

		1293		0.5718

		1292		0.5719

		1291		0.572

		1290		0.5721

		1289		0.5722

		1288		0.5723

		1287		0.5724

		1286		0.5725

		1285		0.5726

		1284		0.5727

		1283		0.5728

		1282		0.5729

		1281		0.5729

		1280		0.573

		1279		0.5731

		1278		0.5731

		1277		0.5732

		1276		0.5732

		1275		0.5733

		1274		0.5734

		1273		0.5734

		1272		0.5735

		1271		0.5736

		1270		0.5736

		1269		0.5737

		1268		0.5738

		1267		0.5739

		1266		0.574

		1265		0.5742

		1264		0.5743

		1263		0.5744

		1262		0.5746

		1261		0.5747

		1260		0.5749

		1259		0.575

		1258		0.5752

		1257		0.5753

		1256		0.5755

		1255		0.5757

		1254		0.5758

		1253		0.576

		1252		0.5762

		1251		0.5764

		1250		0.5765

		1249		0.5767

		1248		0.5769

		1247		0.5771

		1246		0.5773

		1245		0.5775

		1244		0.5777

		1243		0.578

		1242		0.5782

		1241		0.5785

		1240		0.5787

		1239		0.579

		1238		0.5794

		1237		0.5797

		1236		0.5801

		1235		0.5805

		1234		0.5809

		1233		0.5814

		1232		0.5819

		1231		0.5824

		1230		0.5829

		1229		0.5835

		1228		0.5841

		1227		0.5847

		1226		0.5853

		1225		0.5859

		1224		0.5865

		1223		0.5871

		1222		0.5877

		1221		0.5883

		1220		0.5888

		1219		0.5893

		1218		0.5898

		1217		0.5902

		1216		0.5906

		1215		0.5909

		1214		0.5911

		1213		0.5913

		1212		0.5915

		1211		0.5916

		1210		0.5916

		1209		0.5916

		1208		0.5915

		1207		0.5914

		1206		0.5913

		1205		0.5911

		1204		0.5909

		1203		0.5907

		1202		0.5904

		1201		0.5901

		1200		0.5899

		1199		0.5896

		1198		0.5893

		1197		0.5891

		1196		0.5888

		1195		0.5885

		1194		0.5883

		1193		0.588

		1192		0.5877

		1191		0.5875

		1190		0.5872

		1189		0.5869

		1188		0.5867

		1187		0.5865

		1186		0.5862

		1185		0.586

		1184		0.5857

		1183		0.5855

		1182		0.5853

		1181		0.585

		1180		0.5848

		1179		0.5846

		1178		0.5844

		1177		0.5842

		1176		0.584

		1175		0.5838

		1174		0.5836

		1173		0.5835

		1172		0.5833

		1171		0.5832

		1170		0.583

		1169		0.5829

		1168		0.5828

		1167		0.5826

		1166		0.5825

		1165		0.5824

		1164		0.5823

		1163		0.5822

		1162		0.5821

		1161		0.582

		1160		0.5818

		1159		0.5817

		1158		0.5816

		1157		0.5815

		1156		0.5814

		1155		0.5813

		1154		0.5812

		1153		0.5811

		1152		0.581

		1151		0.581

		1150		0.5809

		1149		0.5808

		1148		0.5807

		1147		0.5806

		1146		0.5806

		1145		0.5805

		1144		0.5805

		1143		0.5804

		1142		0.5804

		1141		0.5804

		1140		0.5804

		1139		0.5803

		1138		0.5803

		1137		0.5803

		1136		0.5803

		1135		0.5802

		1134		0.5802

		1133		0.5802

		1132		0.5802

		1131		0.5802

		1130		0.5802

		1129		0.5803

		1128		0.5803

		1127		0.5803

		1126		0.5803

		1125		0.5803

		1124		0.5803

		1123		0.5804

		1122		0.5804

		1121		0.5804

		1120		0.5805

		1119		0.5805

		1118		0.5806

		1117		0.5806

		1116		0.5806

		1115		0.5807

		1114		0.5808

		1113		0.5808

		1112		0.5808

		1111		0.5809

		1110		0.5809

		1109		0.581

		1108		0.581

		1107		0.5811

		1106		0.5811

		1105		0.5812

		1104		0.5812

		1103		0.5813

		1102		0.5813

		1101		0.5813

		1100		0.5814

		1099		0.5814

		1098		0.5814

		1097		0.5815

		1096		0.5815

		1095		0.5816

		1094		0.5816

		1093		0.5816

		1092		0.5817

		1091		0.5817

		1090		0.5818

		1089		0.5818

		1088		0.5819

		1087		0.5819

		1086		0.5819

		1085		0.582

		1084		0.582

		1083		0.5821

		1082		0.5821

		1081		0.5822

		1080		0.5822

		1079		0.5822

		1078		0.5823

		1077		0.5823

		1076		0.5824

		1075		0.5824

		1074		0.5825

		1073		0.5825

		1072		0.5825

		1071		0.5826

		1070		0.5826

		1069		0.5827

		1068		0.5827

		1067		0.5828

		1066		0.5828

		1065		0.5829

		1064		0.5829

		1063		0.583

		1062		0.583

		1061		0.5831

		1060		0.5831

		1059		0.5831

		1058		0.5832

		1057		0.5832

		1056		0.5833

		1055		0.5833

		1054		0.5834

		1053		0.5834

		1052		0.5835

		1051		0.5835

		1050		0.5836

		1049		0.5836

		1048		0.5836

		1047		0.5837

		1046		0.5837

		1045		0.5838

		1044		0.5838

		1043		0.5839

		1042		0.5839

		1041		0.5839

		1040		0.584

		1039		0.584

		1038		0.584

		1037		0.584

		1036		0.584

		1035		0.584

		1034		0.5841

		1033		0.5841

		1032		0.584

		1031		0.5841

		1030		0.5841

		1029		0.5841

		1028		0.5841

		1027		0.5841

		1026		0.5841

		1025		0.5841

		1024		0.5841

		1023		0.5841

		1022		0.5841

		1021		0.5841

		1020		0.5841

		1019		0.5841

		1018		0.5841

		1017		0.5841

		1016		0.5841

		1015		0.5841

		1014		0.5841

		1013		0.5841

		1012		0.584

		1011		0.584

		1010		0.584

		1009		0.5839

		1008		0.5839

		1007		0.5838

		1006		0.5837

		1005		0.5837

		1004		0.5836

		1003		0.5835

		1002		0.5834

		1001		0.5833

		1000		0.5832

		999		0.5831

		998		0.583

		997		0.5829

		996		0.5827

		995		0.5826

		994		0.5824

		993		0.5823

		992		0.5821

		991		0.5819

		990		0.5818

		989		0.5816

		988		0.5813

		987		0.5811

		986		0.5809

		985		0.5806

		984		0.5804

		983		0.5801

		982		0.5799

		981		0.5796

		980		0.5793

		979		0.579

		978		0.5787

		977		0.5783

		976		0.578

		975		0.5777

		974		0.5773

		973		0.5769

		972		0.5765

		971		0.5762

		970		0.5758

		969		0.5754

		968		0.5749

		967		0.5745

		966		0.5741

		965		0.5736

		964		0.5732

		963		0.5728

		962		0.5723

		961		0.5719

		960		0.5714

		959		0.571

		958		0.5706

		957		0.5702

		956		0.5698

		955		0.5694

		954		0.5691

		953		0.5687

		952		0.5684

		951		0.5681

		950		0.5678

		949		0.5676

		948		0.5674

		947		0.5672

		946		0.567

		945		0.5668

		944		0.5667

		943		0.5666

		942		0.5665

		941		0.5665

		940		0.5664

		939		0.5664

		938		0.5664

		937		0.5665

		936		0.5665

		935		0.5666

		934		0.5666

		933		0.5667

		932		0.5667

		931		0.5668

		930		0.5669

		929		0.5669

		928		0.567

		927		0.5671

		926		0.5672

		925		0.5673

		924		0.5674

		923		0.5674

		922		0.5675

		921		0.5675

		920		0.5675

		919		0.5675

		918		0.5676

		917		0.5676

		916		0.5676

		915		0.5676

		914		0.5677

		913		0.5677

		912		0.5677

		911		0.5677

		910		0.5677

		909		0.5677

		908		0.5678

		907		0.5678

		906		0.5678

		905		0.5678

		904		0.5678

		903		0.5678

		902		0.5678

		901		0.5678

		900		0.5678

		899		0.5678

		898		0.5678

		897		0.5678

		896		0.5677

		895		0.5677

		894		0.5677

		893		0.5677

		892		0.5677

		891		0.5676

		890		0.5676

		889		0.5676

		888		0.5676

		887		0.5675

		886		0.5676

		885		0.5676

		884		0.5676

		883		0.5676

		882		0.5677

		881		0.5677

		880		0.5678

		879		0.5679

		878		0.568

		877		0.5681

		876		0.5683

		875		0.5685

		874		0.5688

		873		0.5692

		872		0.5697

		871		0.5702

		870		0.5709

		869		0.5716

		868		0.5724

		867		0.5732

		866		0.5742

		865		0.5752

		864		0.5762

		863		0.5774

		862		0.5786

		861		0.5799

		860		0.5813

		859		0.5826

		858		0.5839

		857		0.5851

		856		0.5862

		855		0.5873

		854		0.5883

		853		0.5892

		852		0.5901

		851		0.5908

		850		0.5915

		849		0.5921

		848		0.5927

		847		0.5931

		846		0.5935

		845		0.5938

		844		0.594

		843		0.5941

		842		0.5942

		841		0.5942

		840		0.5943

		839		0.5943

		838		0.5943

		837		0.5943

		836		0.5942

		835		0.5942

		834		0.5941

		833		0.594

		832		0.594

		831		0.5939

		830		0.5937

		829		0.5936

		828		0.5935

		827		0.5934

		826		0.5933

		825		0.5932

		824		0.5931

		823		0.593

		822		0.593

		821		0.5929

		820		0.5928

		819		0.5928

		818		0.5927

		817		0.5927

		816		0.5926

		815		0.5926

		814		0.5925

		813		0.5925

		812		0.5925

		811		0.5925

		810		0.5925

		809		0.5925

		808		0.5925

		807		0.5925

		806		0.5925

		805		0.5925

		804		0.5925

		803		0.5926

		802		0.5926

		801		0.5927

		800		0.5928

		799		0.5928

		798		0.5929

		797		0.593

		796		0.5931

		795		0.5932

		794		0.5932

		793		0.5933

		792		0.5933

		791		0.5934

		790		0.5935

		789		0.5936

		788		0.5936

		787		0.5937

		786		0.5937

		785		0.5938

		784		0.5938

		783		0.5938

		782		0.5938

		781		0.5938

		780		0.5939

		779		0.5939

		778		0.5939

		777		0.5939

		776		0.5939

		775		0.5939

		774		0.5939

		773		0.5939

		772		0.5939

		771		0.5939

		770		0.594

		769		0.594

		768		0.594

		767		0.594

		766		0.5941

		765		0.5941

		764		0.5942

		763		0.5942

		762		0.5943

		761		0.5943

		760		0.5943

		759		0.5944

		758		0.5944

		757		0.5944

		756		0.5945

		755		0.5945

		754		0.5945

		753		0.5945

		752		0.5945

		751		0.5945

		750		0.5945

		749		0.5944

		748		0.5944

		747		0.5944

		746		0.5943

		745		0.5943

		744		0.5943

		743		0.5942

		742		0.5942

		741		0.5942

		740		0.5942

		739		0.5941

		738		0.5941

		737		0.5941

		736		0.5941

		735		0.5941

		734		0.5941

		733		0.5941

		732		0.5941

		731		0.5941

		730		0.5942

		729		0.5942

		728		0.5942

		727		0.5943

		726		0.5943

		725		0.5943

		724		0.5944

		723		0.5944

		722		0.5944

		721		0.5945

		720		0.5945

		719		0.5945

		718		0.5945

		717		0.5946

		716		0.5946

		715		0.5946

		714		0.5946

		713		0.5946

		712		0.5947

		711		0.5947

		710		0.5947

		709		0.5947

		708		0.5947

		707		0.5948

		706		0.5948

		705		0.5948

		704		0.5948

		703		0.5948

		702		0.5949

		701		0.5949

		700		0.5949

		699		0.5949

		698		0.5949

		697		0.5949

		696		0.5949

		695		0.5949

		694		0.5949

		693		0.5949

		692		0.5949

		691		0.5949

		690		0.5949

		689		0.5949

		688		0.595

		687		0.595

		686		0.595

		685		0.595

		684		0.5951

		683		0.5951

		682		0.5951

		681		0.5952

		680		0.5952

		679		0.5953

		678		0.5953

		677		0.5954

		676		0.5954

		675		0.5954

		674		0.5955

		673		0.5955

		672		0.5955

		671		0.5955

		670		0.5955

		669		0.5955

		668		0.5955

		667		0.5955

		666		0.5955

		665		0.5955

		664		0.5955

		663		0.5955

		662		0.5955

		661		0.5955

		660		0.5955

		659		0.5955

		658		0.5955

		657		0.5956

		656		0.5956

		655		0.5956

		654		0.5956

		653		0.5957

		652		0.5957

		651		0.5957

		650		0.5958

		649		0.5958

		648		0.5958

		647		0.5958

		646		0.5959

		645		0.5959

		644		0.5959

		643		0.5959

		642		0.5959

		641		0.5959

		640		0.5959

		639		0.5959

		638		0.5959

		637		0.5959

		636		0.5959

		635		0.5959

		634		0.5959

		633		0.5959

		632		0.5959

		631		0.596

		630		0.596

		629		0.596

		628		0.596

		627		0.5961

		626		0.5961

		625		0.5962

		624		0.5962

		623		0.5962

		622		0.5963

		621		0.5963

		620		0.5964

		619		0.5965

		618		0.5965

		617		0.5965

		616		0.5966

		615		0.5966

		614		0.5966

		613		0.5967

		612		0.5967

		611		0.5967

		610		0.5967

		609		0.5968

		608		0.5968

		607		0.5968

		606		0.5968

		605		0.5968

		604		0.5968

		603		0.5968

		602		0.5968

		601		0.5968

		600		0.5968

		599		0.5968

		598		0.5967

		597		0.5967

		596		0.5967

		595		0.5967

		594		0.5967

		593		0.5967

		592		0.5967

		591		0.5967

		590		0.5967

		589		0.5967

		588		0.5967

		587		0.5967

		586		0.5967

		585		0.5967

		584		0.5967

		583		0.5967

		582		0.5967

		581		0.5967

		580		0.5967

		579		0.5967

		578		0.5967

		577		0.5967

		576		0.5967

		575		0.5967

		574		0.5967

		573		0.5967

		572		0.5966

		571		0.5966

		570		0.5966

		569		0.5966

		568		0.5966

		567		0.5966

		566		0.5966

		565		0.5966

		564		0.5965

		563		0.5965

		562		0.5966

		561		0.5966

		560		0.5966

		559		0.5966

		558		0.5966

		557		0.5967

		556		0.5967

		555		0.5967

		554		0.5968

		553		0.5968

		552		0.5969

		551		0.5969

		550		0.5969

		549		0.597

		548		0.597

		547		0.5971

		546		0.5972

		545		0.5972

		544		0.5973

		543		0.5974

		542		0.5974

		541		0.5975

		540		0.5976

		539		0.5977

		538		0.5978

		537		0.5979

		536		0.598

		535		0.5981

		534		0.5982

		533		0.5984

		532		0.5986

		531		0.5987

		530		0.5989

		529		0.5991

		528		0.5994

		527		0.5996

		526		0.5998

		525		0.6

		524		0.6003

		523		0.6005

		522		0.6008

		521		0.601

		520		0.6013

		519		0.6015

		518		0.6018

		517		0.602

		516		0.6022

		515		0.6023

		514		0.6025

		513		0.6026

		512		0.6027

		511		0.6028

		510		0.6029

		509		0.6029

		508		0.6029

		507		0.6029

		506		0.6028

		505		0.6028

		504		0.6027

		503		0.6026

		502		0.6025

		501		0.6024

		500		0.6022

		499		0.6021

		498		0.602

		497		0.6018

		496		0.6017

		495		0.6015

		494		0.6014

		493		0.6012

		492		0.6011

		491		0.601

		490		0.6009

		489		0.6008

		488		0.6007

		487		0.6007

		486		0.6006

		485		0.6006

		484		0.6006

		483		0.6006

		482		0.6007

		481		0.6008

		480		0.6009

		479		0.601

		478		0.6011

		477		0.6013

		476		0.6014

		475		0.6016

		474		0.6018

		473		0.602

		472		0.6021

		471		0.6023

		470		0.6025

		469		0.6026

		468		0.6028

		467		0.6029

		466		0.603

		465		0.6031

		464		0.6032

		463		0.6032

		462		0.6033

		461		0.6033

		460		0.6034

		459		0.6034

		458		0.6034

		457		0.6033

		456		0.6033

		455		0.6033

		454		0.6033

		453		0.6032

		452		0.6032

		451		0.6031

		450		0.6031

		449		0.6031

		448		0.603

		447		0.603

		446		0.6029

		445		0.6029

		444		0.6029

		443		0.6029

		442		0.6028

		441		0.6028

		440		0.6028

		439		0.6028

		438		0.6027

		437		0.6027

		436		0.6027

		435		0.6027

		434		0.6027

		433		0.6027

		432		0.6026

		431		0.6026

		430		0.6026

		429		0.6026

		428		0.6025

		427		0.6025

		426		0.6024

		425		0.6024

		424		0.6023

		423		0.6023

		422		0.6022

		421		0.6021

		420		0.6021

		419		0.602

		418		0.6019

		417		0.6018

		416		0.6017

		415		0.6016

		414		0.6015

		413		0.6014

		412		0.6013

		411		0.6012

		410		0.6011

		409		0.601

		408		0.6009

		407		0.6007

		406		0.6006

		405		0.6005

		404		0.6003

		403		0.6002

		402		0.6

		401		0.5998

		400		0.5997

		399		0.5995

		398		0.5993

		397		0.5991

		396		0.5989

		395		0.5987

		394		0.5984

		393		0.5981

		392		0.5978

		391		0.5975

		390		0.5972

		389		0.5969

		388		0.5966

		387		0.5962

		386		0.5959

		385		0.5956

		384		0.5953

		383		0.5949

		382		0.5945

		381		0.594

		380		0.5936

		379		0.5932

		378		0.5928

		377		0.5924

		376		0.5921

		375		0.5917

		374		0.5914

		373		0.5911

		372		0.5906

		371		0.5901

		370		0.5896

		369		0.589

		368		0.5884

		367		0.5879

		366		0.5874

		365		0.5868

		364		0.5863

		363		0.5857

		362		0.5851

		361		0.5845

		360		0.5839

		359		0.5832

		358		0.5824

		357		0.5816

		356		0.5809

		355		0.5802

		354		0.5796

		353		0.5791

		352		0.5786

		351		0.5781

		350		0.5776

		349		0.5771

		348		0.5766

		347		0.5761

		346		0.5757

		345		0.5753

		344		0.5749

		343		0.5745

		342		0.5741

		341		0.574

		340		0.5739

		339		0.5738

		338		0.5737

		337		0.5735

		336		0.5733

		335		0.5732

		334		0.5731

		333		0.573

		332		0.573

		331		0.573

		330		0.5731

		329		0.5732

		328		0.5734

		327		0.5735

		326		0.5737

		325		0.5738

		324		0.5738

		323		0.5738

		322		0.5738

		321		0.5739

		320		0.5739

		319		0.5739

		318		0.574

		317		0.5741

		316		0.5741

		315		0.5741

		314		0.5741

		313		0.574

		312		0.5739

		311		0.5738

		310		0.5736

		309		0.5735

		308		0.5734

		307		0.5732

		306		0.5731

		305		0.5729

		304		0.5727

		303		0.5724

		302		0.5721

		301		0.5718

		300		0.5714

		299		0.5711

		298		0.5706

		297		0.5702

		296		0.5697

		295		0.5692

		294		0.5686

		293		0.568

		292		0.5674

		291		0.5667

		290		0.566

		289		0.5653

		288		0.5646

		287		0.5638

		286		0.563

		285		0.5622

		284		0.5614

		283		0.5605

		282		0.5597

		281		0.5588

		280		0.5579

		279		0.5571

		278		0.5562

		277		0.5553

		276		0.5543

		275		0.5534

		274		0.5524

		273		0.5515

		272		0.5504

		271		0.5494

		270		0.5483

		269		0.5472

		268		0.5461

		267		0.5449

		266		0.5436

		265		0.5423

		264		0.541

		263		0.5396

		262		0.5382

		261		0.5368

		260		0.5354

		259		0.5339

		258		0.5324

		257		0.5309

		256		0.5293

		255		0.5278

		254		0.5263

		253		0.5247

		252		0.5231

		251		0.5216

		250		0.52
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		nm		A

		1400		0.439

		1399		0.4393

		1398		0.4395

		1397		0.4398

		1396		0.44

		1395		0.4402

		1394		0.4404

		1393		0.4405

		1392		0.4407

		1391		0.4407

		1390		0.4408

		1389		0.4408

		1388		0.4408

		1387		0.4407

		1386		0.4406

		1385		0.4405

		1384		0.4404

		1383		0.4403

		1382		0.4402

		1381		0.4401

		1380		0.4399

		1379		0.4398

		1378		0.4397

		1377		0.4396

		1376		0.4395

		1375		0.4395

		1374		0.4394

		1373		0.4393

		1372		0.4393

		1371		0.4393

		1370		0.4392

		1369		0.4392

		1368		0.4392

		1367		0.4392

		1366		0.4391

		1365		0.4391

		1364		0.4391

		1363		0.4391

		1362		0.4391

		1361		0.4391

		1360		0.4391

		1359		0.4391

		1358		0.4391

		1357		0.4391

		1356		0.4392

		1355		0.4392

		1354		0.4393

		1353		0.4393

		1352		0.4394

		1351		0.4395

		1350		0.4396

		1349		0.4397

		1348		0.4398

		1347		0.4399

		1346		0.44

		1345		0.4401

		1344		0.4402

		1343		0.4403

		1342		0.4405

		1341		0.4406

		1340		0.4407

		1339		0.4408

		1338		0.4409

		1337		0.441

		1336		0.4411

		1335		0.4412

		1334		0.4413

		1333		0.4414

		1332		0.4415

		1331		0.4415

		1330		0.4416

		1329		0.4417

		1328		0.4418

		1327		0.4418

		1326		0.4419

		1325		0.4419

		1324		0.442

		1323		0.442

		1322		0.442

		1321		0.4421

		1320		0.4421

		1319		0.4421

		1318		0.4421

		1317		0.4421

		1316		0.4422

		1315		0.4422

		1314		0.4422

		1313		0.4422

		1312		0.4422

		1311		0.4422

		1310		0.4423

		1309		0.4423

		1308		0.4424

		1307		0.4424

		1306		0.4424

		1305		0.4425

		1304		0.4425

		1303		0.4426

		1302		0.4427

		1301		0.4427

		1300		0.4428

		1299		0.4429

		1298		0.443

		1297		0.4431

		1296		0.4431

		1295		0.4432

		1294		0.4433

		1293		0.4434

		1292		0.4435

		1291		0.4436

		1290		0.4437

		1289		0.4438

		1288		0.4439

		1287		0.4439

		1286		0.444

		1285		0.4441

		1284		0.4442

		1283		0.4442

		1282		0.4443

		1281		0.4444

		1280		0.4444

		1279		0.4445

		1278		0.4445

		1277		0.4446

		1276		0.4446

		1275		0.4447

		1274		0.4447

		1273		0.4448

		1272		0.4448

		1271		0.4448

		1270		0.4449

		1269		0.445

		1268		0.445

		1267		0.4451

		1266		0.4452

		1265		0.4453

		1264		0.4453

		1263		0.4454

		1262		0.4456

		1261		0.4457

		1260		0.4458

		1259		0.4459

		1258		0.4461

		1257		0.4463

		1256		0.4464

		1255		0.4466

		1254		0.4468

		1253		0.447

		1252		0.4472

		1251		0.4474

		1250		0.4476

		1249		0.4478

		1248		0.448

		1247		0.4483

		1246		0.4486

		1245		0.4489

		1244		0.4492

		1243		0.4495

		1242		0.4498

		1241		0.4502

		1240		0.4506

		1239		0.451

		1238		0.4515

		1237		0.452

		1236		0.4525

		1235		0.4531

		1234		0.4537

		1233		0.4544

		1232		0.4551

		1231		0.4558

		1230		0.4565

		1229		0.4573

		1228		0.4581

		1227		0.4589

		1226		0.4597

		1225		0.4606

		1224		0.4614

		1223		0.4622

		1222		0.4629

		1221		0.4637

		1220		0.4644

		1219		0.465

		1218		0.4656

		1217		0.4661

		1216		0.4665

		1215		0.4669

		1214		0.4671

		1213		0.4673

		1212		0.4674

		1211		0.4675

		1210		0.4674

		1209		0.4673

		1208		0.4671

		1207		0.4669

		1206		0.4666

		1205		0.4663

		1204		0.4659

		1203		0.4655

		1202		0.465

		1201		0.4646

		1200		0.4641

		1199		0.4636

		1198		0.4631

		1197		0.4627

		1196		0.4622

		1195		0.4617

		1194		0.4612

		1193		0.4607

		1192		0.4602

		1191		0.4598

		1190		0.4593

		1189		0.4588

		1188		0.4584

		1187		0.4579

		1186		0.4575

		1185		0.457

		1184		0.4566

		1183		0.4561

		1182		0.4557

		1181		0.4552

		1180		0.4548

		1179		0.4544

		1178		0.454

		1177		0.4536

		1176		0.4532

		1175		0.4528

		1174		0.4525

		1173		0.4521

		1172		0.4518

		1171		0.4515

		1170		0.4511

		1169		0.4508

		1168		0.4506

		1167		0.4503

		1166		0.45

		1165		0.4498

		1164		0.4495

		1163		0.4493

		1162		0.449

		1161		0.4488

		1160		0.4486

		1159		0.4484

		1158		0.4482

		1157		0.448

		1156		0.4478

		1155		0.4476

		1154		0.4474

		1153		0.4472

		1152		0.447

		1151		0.4468

		1150		0.4466

		1149		0.4464

		1148		0.4463

		1147		0.4461

		1146		0.4459

		1145		0.4458

		1144		0.4456

		1143		0.4455

		1142		0.4453

		1141		0.4452

		1140		0.4451

		1139		0.4449

		1138		0.4448

		1137		0.4447

		1136		0.4446

		1135		0.4445

		1134		0.4444

		1133		0.4443

		1132		0.4442

		1131		0.4441

		1130		0.444

		1129		0.4439

		1128		0.4439

		1127		0.4438

		1126		0.4437

		1125		0.4437

		1124		0.4436

		1123		0.4436

		1122		0.4435

		1121		0.4435

		1120		0.4435

		1119		0.4434

		1118		0.4434

		1117		0.4434

		1116		0.4434

		1115		0.4433

		1114		0.4433

		1113		0.4433

		1112		0.4433

		1111		0.4433

		1110		0.4433

		1109		0.4432

		1108		0.4432

		1107		0.4432

		1106		0.4432

		1105		0.4432

		1104		0.4432

		1103		0.4431

		1102		0.4431

		1101		0.4431

		1100		0.4431

		1099		0.4431

		1098		0.443

		1097		0.443

		1096		0.443

		1095		0.4429

		1094		0.4429

		1093		0.4429

		1092		0.4428

		1091		0.4428

		1090		0.4428

		1089		0.4428

		1088		0.4427

		1087		0.4427

		1086		0.4427

		1085		0.4426

		1084		0.4426

		1083		0.4426

		1082		0.4426

		1081		0.4425

		1080		0.4425

		1079		0.4425

		1078		0.4425

		1077		0.4425

		1076		0.4425

		1075		0.4425

		1074		0.4425

		1073		0.4425

		1072		0.4425

		1071		0.4425

		1070		0.4425

		1069		0.4425

		1068		0.4425

		1067		0.4425

		1066		0.4425

		1065		0.4425

		1064		0.4425

		1063		0.4425

		1062		0.4425

		1061		0.4426

		1060		0.4425

		1059		0.4426

		1058		0.4426

		1057		0.4426

		1056		0.4426

		1055		0.4426

		1054		0.4426

		1053		0.4426

		1052		0.4426

		1051		0.4426

		1050		0.4426

		1049		0.4426

		1048		0.4426

		1047		0.4426

		1046		0.4426

		1045		0.4426

		1044		0.4426

		1043		0.4426

		1042		0.4426

		1041		0.4426

		1040		0.4426

		1039		0.4426

		1038		0.4426

		1037		0.4426

		1036		0.4426

		1035		0.4426

		1034		0.4425

		1033		0.4425

		1032		0.4425

		1031		0.4425

		1030		0.4425

		1029		0.4425

		1028		0.4424

		1027		0.4424

		1026		0.4424

		1025		0.4424

		1024		0.4424

		1023		0.4424

		1022		0.4424

		1021		0.4424

		1020		0.4424

		1019		0.4423

		1018		0.4423

		1017		0.4423

		1016		0.4423

		1015		0.4423

		1014		0.4423

		1013		0.4423

		1012		0.4423

		1011		0.4423

		1010		0.4423

		1009		0.4423

		1008		0.4423

		1007		0.4422

		1006		0.4422

		1005		0.4422

		1004		0.4422

		1003		0.4422

		1002		0.4422

		1001		0.4422

		1000		0.4421

		999		0.4421

		998		0.4421

		997		0.4421

		996		0.4421

		995		0.4421

		994		0.4421

		993		0.4421

		992		0.442

		991		0.442

		990		0.442

		989		0.442

		988		0.442

		987		0.4419

		986		0.4419

		985		0.4419

		984		0.4419

		983		0.4418

		982		0.4418

		981		0.4417

		980		0.4417

		979		0.4416

		978		0.4415

		977		0.4415

		976		0.4414

		975		0.4413

		974		0.4413

		973		0.4412

		972		0.4411

		971		0.441

		970		0.441

		969		0.4409

		968		0.4409

		967		0.4408

		966		0.4407

		965		0.4407

		964		0.4407

		963		0.4406

		962		0.4406

		961		0.4405

		960		0.4405

		959		0.4404

		958		0.4404

		957		0.4403

		956		0.4403

		955		0.4402

		954		0.4402

		953		0.4401

		952		0.4401

		951		0.44

		950		0.44

		949		0.4399

		948		0.4399

		947		0.4399

		946		0.4399

		945		0.4399

		944		0.4399

		943		0.4399

		942		0.4399

		941		0.4399

		940		0.44

		939		0.44

		938		0.4401

		937		0.4402

		936		0.4402

		935		0.4403

		934		0.4404

		933		0.4405

		932		0.4407

		931		0.4407

		930		0.4408

		929		0.4409

		928		0.441

		927		0.4411

		926		0.4412

		925		0.4413

		924		0.4414

		923		0.4415

		922		0.4415

		921		0.4416

		920		0.4416

		919		0.4417

		918		0.4417

		917		0.4417

		916		0.4418

		915		0.4418

		914		0.4418

		913		0.4418

		912		0.4418

		911		0.4418

		910		0.4418

		909		0.4418

		908		0.4418

		907		0.4418

		906		0.4417

		905		0.4417

		904		0.4417

		903		0.4417

		902		0.4417

		901		0.4417

		900		0.4417

		899		0.4416

		898		0.4416

		897		0.4416

		896		0.4416

		895		0.4416

		894		0.4416

		893		0.4416

		892		0.4416

		891		0.4416

		890		0.4416

		889		0.4416

		888		0.4417

		887		0.4417

		886		0.4417

		885		0.4418

		884		0.4418

		883		0.4419

		882		0.442

		881		0.442

		880		0.4421

		879		0.4421

		878		0.4422

		877		0.4423

		876		0.4424

		875		0.4425

		874		0.4426

		873		0.4427

		872		0.4429

		871		0.4431

		870		0.4433

		869		0.4436

		868		0.4438

		867		0.4441

		866		0.4444

		865		0.4448

		864		0.4452

		863		0.4456

		862		0.4461

		861		0.4465

		860		0.447

		859		0.4475

		858		0.448

		857		0.4484

		856		0.4489

		855		0.4493

		854		0.4497

		853		0.4501

		852		0.4504

		851		0.4507

		850		0.4509

		849		0.4512

		848		0.4513

		847		0.4515

		846		0.4516

		845		0.4516

		844		0.4517

		843		0.4517

		842		0.4517

		841		0.4516

		840		0.4515

		839		0.4514

		838		0.4514

		837		0.4513

		836		0.4512

		835		0.4512

		834		0.4511

		833		0.451

		832		0.451

		831		0.4509

		830		0.4508

		829		0.4508

		828		0.4507

		827		0.4507

		826		0.4506

		825		0.4506

		824		0.4506

		823		0.4507

		822		0.4507

		821		0.4507

		820		0.4507

		819		0.4507

		818		0.4507

		817		0.4507

		816		0.4507

		815		0.4507

		814		0.4508

		813		0.4508

		812		0.4508

		811		0.4509

		810		0.4509

		809		0.4509

		808		0.4509

		807		0.451

		806		0.451

		805		0.451

		804		0.451

		803		0.4511

		802		0.4511

		801		0.4512

		800		0.4512

		799		0.4512

		798		0.4513

		797		0.4513

		796		0.4513

		795		0.4514

		794		0.4514

		793		0.4515

		792		0.4515

		791		0.4515

		790		0.4516

		789		0.4516

		788		0.4516

		787		0.4516

		786		0.4516

		785		0.4516

		784		0.4516

		783		0.4516

		782		0.4515

		781		0.4515

		780		0.4515

		779		0.4515

		778		0.4514

		777		0.4513

		776		0.4513

		775		0.4512

		774		0.4512

		773		0.4512

		772		0.4511

		771		0.4511

		770		0.4511

		769		0.4511

		768		0.4511

		767		0.4511

		766		0.4512

		765		0.4512

		764		0.4512

		763		0.4513

		762		0.4513

		761		0.4513

		760		0.4514

		759		0.4515

		758		0.4515

		757		0.4516

		756		0.4516

		755		0.4516

		754		0.4517

		753		0.4517

		752		0.4517

		751		0.4517

		750		0.4517

		749		0.4517

		748		0.4518

		747		0.4518

		746		0.4518

		745		0.4518

		744		0.4518

		743		0.4519

		742		0.4519

		741		0.4519

		740		0.4519

		739		0.4519

		738		0.4519

		737		0.4519

		736		0.4519

		735		0.452

		734		0.452

		733		0.452

		732		0.452

		731		0.452

		730		0.452

		729		0.452

		728		0.4521

		727		0.4521

		726		0.4521

		725		0.4521

		724		0.4521

		723		0.4522

		722		0.4522

		721		0.4522

		720		0.4523

		719		0.4523

		718		0.4523

		717		0.4524

		716		0.4524

		715		0.4524

		714		0.4524

		713		0.4525

		712		0.4525

		711		0.4525

		710		0.4525

		709		0.4525

		708		0.4525

		707		0.4525

		706		0.4525

		705		0.4525

		704		0.4525

		703		0.4525

		702		0.4525

		701		0.4525

		700		0.4525

		699		0.4525

		698		0.4525

		697		0.4525

		696		0.4526

		695		0.4526

		694		0.4526

		693		0.4526

		692		0.4527

		691		0.4527

		690		0.4527

		689		0.4527

		688		0.4528

		687		0.4528

		686		0.4528

		685		0.4529

		684		0.4529

		683		0.453

		682		0.453

		681		0.453

		680		0.453

		679		0.453

		678		0.4531

		677		0.4531

		676		0.4531

		675		0.4531

		674		0.4531

		673		0.4532

		672		0.4532

		671		0.4532

		670		0.4532

		669		0.4532

		668		0.4532

		667		0.4533

		666		0.4533

		665		0.4533

		664		0.4533

		663		0.4533

		662		0.4534

		661		0.4534

		660		0.4534

		659		0.4534

		658		0.4535

		657		0.4535

		656		0.4535

		655		0.4535

		654		0.4536

		653		0.4536

		652		0.4536

		651		0.4537

		650		0.4537

		649		0.4537

		648		0.4537

		647		0.4538

		646		0.4538

		645		0.4538

		644		0.4538

		643		0.4538

		642		0.4538

		641		0.4538

		640		0.4538

		639		0.4538

		638		0.4539

		637		0.4539

		636		0.4539

		635		0.4539

		634		0.4539

		633		0.4539

		632		0.4539

		631		0.4539

		630		0.4539

		629		0.4539

		628		0.4539

		627		0.454

		626		0.454

		625		0.454

		624		0.4541

		623		0.4541

		622		0.4541

		621		0.4542

		620		0.4542

		619		0.4543

		618		0.4543

		617		0.4543

		616		0.4544

		615		0.4544

		614		0.4544

		613		0.4544

		612		0.4545

		611		0.4545

		610		0.4545

		609		0.4545

		608		0.4545

		607		0.4545

		606		0.4546

		605		0.4546

		604		0.4546

		603		0.4546

		602		0.4546

		601		0.4546

		600		0.4546

		599		0.4547

		598		0.4547

		597		0.4547

		596		0.4547

		595		0.4548

		594		0.4548

		593		0.4548

		592		0.4548

		591		0.4549

		590		0.4549

		589		0.4549

		588		0.4549

		587		0.455

		586		0.455

		585		0.455

		584		0.455

		583		0.455

		582		0.4551

		581		0.4551

		580		0.4551

		579		0.4551

		578		0.4551

		577		0.4551

		576		0.4551

		575		0.4551

		574		0.455

		573		0.455

		572		0.455

		571		0.455

		570		0.455

		569		0.455

		568		0.4549

		567		0.4549

		566		0.4549

		565		0.4549

		564		0.4549

		563		0.4549

		562		0.4549

		561		0.4548

		560		0.4549

		559		0.4549

		558		0.4549

		557		0.4549

		556		0.4549

		555		0.455

		554		0.455

		553		0.455

		552		0.4551

		551		0.4551

		550		0.4552

		549		0.4553

		548		0.4553

		547		0.4554

		546		0.4555

		545		0.4556

		544		0.4557

		543		0.4558

		542		0.4559

		541		0.456

		540		0.4561

		539		0.4563

		538		0.4564

		537		0.4565

		536		0.4567

		535		0.4569

		534		0.457

		533		0.4572

		532		0.4574

		531		0.4576

		530		0.4578

		529		0.4581

		528		0.4583

		527		0.4585

		526		0.4588

		525		0.459

		524		0.4593

		523		0.4595

		522		0.4597

		521		0.46

		520		0.4602

		519		0.4604

		518		0.4606

		517		0.4608

		516		0.4609

		515		0.4611

		514		0.4612

		513		0.4613

		512		0.4613

		511		0.4614

		510		0.4614

		509		0.4614

		508		0.4613

		507		0.4613

		506		0.4612

		505		0.4612

		504		0.4611

		503		0.461

		502		0.4608

		501		0.4607

		500		0.4606

		499		0.4605

		498		0.4603

		497		0.4602

		496		0.4601

		495		0.4599

		494		0.4598

		493		0.4597

		492		0.4596

		491		0.4596

		490		0.4595

		489		0.4595

		488		0.4594

		487		0.4594

		486		0.4595

		485		0.4595

		484		0.4596

		483		0.4597

		482		0.4598

		481		0.46

		480		0.4601

		479		0.4603

		478		0.4605

		477		0.4607

		476		0.4609

		475		0.4611

		474		0.4614

		473		0.4616

		472		0.4618

		471		0.462

		470		0.4621

		469		0.4623

		468		0.4625

		467		0.4626

		466		0.4627

		465		0.4628

		464		0.4628

		463		0.4629

		462		0.4629

		461		0.463

		460		0.463

		459		0.463

		458		0.4629

		457		0.4629

		456		0.4629

		455		0.4628

		454		0.4628

		453		0.4628

		452		0.4627

		451		0.4627

		450		0.4626

		449		0.4626

		448		0.4626

		447		0.4625

		446		0.4625

		445		0.4625

		444		0.4624

		443		0.4624

		442		0.4624

		441		0.4624

		440		0.4624

		439		0.4624

		438		0.4624

		437		0.4624

		436		0.4624

		435		0.4624

		434		0.4624

		433		0.4624

		432		0.4624

		431		0.4624

		430		0.4624

		429		0.4624

		428		0.4623

		427		0.4623

		426		0.4623

		425		0.4622

		424		0.4622

		423		0.4621

		422		0.4621

		421		0.462

		420		0.4619

		419		0.4619

		418		0.4618

		417		0.4617

		416		0.4616

		415		0.4616

		414		0.4615

		413		0.4614

		412		0.4613

		411		0.4612

		410		0.4611

		409		0.4609

		408		0.4608

		407		0.4607

		406		0.4606

		405		0.4604

		404		0.4603

		403		0.4601

		402		0.46

		401		0.4598

		400		0.4596

		399		0.4594

		398		0.4592

		397		0.459

		396		0.4588

		395		0.4586

		394		0.4584

		393		0.4581

		392		0.4579

		391		0.4577

		390		0.4575

		389		0.4572

		388		0.457

		387		0.4567

		386		0.4563

		385		0.4559

		384		0.4556

		383		0.4552

		382		0.4548

		381		0.4543

		380		0.4539

		379		0.4534

		378		0.453

		377		0.4526

		376		0.4521

		375		0.4516

		374		0.4511

		373		0.4507

		372		0.4502

		371		0.4498

		370		0.4495

		369		0.4492

		368		0.4489

		367		0.4486

		366		0.4483

		365		0.448

		364		0.4477

		363		0.4474

		362		0.4471

		361		0.4468

		360		0.4465

		359		0.4462

		358		0.4458

		357		0.4454

		356		0.445

		355		0.4446

		354		0.4442

		353		0.4437

		352		0.4432

		351		0.4427

		350		0.4423

		349		0.4419

		348		0.4415

		347		0.4411

		346		0.4407

		345		0.4403

		344		0.4401

		343		0.4398

		342		0.4397

		341		0.4396

		340		0.4396

		339		0.4397

		338		0.4397

		337		0.4398

		336		0.44

		335		0.4402

		334		0.4405

		333		0.4407

		332		0.4409

		331		0.4412

		330		0.4416

		329		0.442

		328		0.4425

		327		0.4429

		326		0.4433

		325		0.4437

		324		0.4439

		323		0.4442

		322		0.4445

		321		0.4448

		320		0.4452

		319		0.4456

		318		0.446

		317		0.4464

		316		0.4467

		315		0.4471

		314		0.4474

		313		0.4478

		312		0.4481

		311		0.4483

		310		0.4486

		309		0.4489

		308		0.4492

		307		0.4495

		306		0.4498

		305		0.4501

		304		0.4503

		303		0.4505

		302		0.4506

		301		0.4507

		300		0.4507

		299		0.4508

		298		0.4508

		297		0.4508

		296		0.4507

		295		0.4506

		294		0.4505

		293		0.4503

		292		0.4501

		291		0.4499

		290		0.4496

		289		0.4493

		288		0.4489

		287		0.4485

		286		0.4481

		285		0.4476

		284		0.4471

		283		0.4466

		282		0.4461

		281		0.4455

		280		0.4449

		279		0.4442

		278		0.4436

		277		0.4429

		276		0.4422

		275		0.4414

		274		0.4406

		273		0.4398

		272		0.4389

		271		0.438

		270		0.437

		269		0.436

		268		0.4349

		267		0.4338

		266		0.4327

		265		0.4315

		264		0.4302

		263		0.4289

		262		0.4276

		261		0.4262

		260		0.4249

		259		0.4234

		258		0.422

		257		0.4206

		256		0.4191

		255		0.4176

		254		0.4162

		253		0.4147

		252		0.4132

		251		0.4116

		250		0.4101
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		nm		A

		1400		0.2036

		1399		0.2058

		1398		0.208

		1397		0.21

		1396		0.2121

		1395		0.2139

		1394		0.2157

		1393		0.2173

		1392		0.2186

		1391		0.2198

		1390		0.2208

		1389		0.2215

		1388		0.222

		1387		0.2223

		1386		0.2224

		1385		0.2223

		1384		0.2221

		1383		0.2217

		1382		0.2211

		1381		0.2204

		1380		0.2196

		1379		0.2188

		1378		0.2178

		1377		0.2168

		1376		0.2158

		1375		0.2148

		1374		0.2138

		1373		0.2128

		1372		0.2119

		1371		0.211

		1370		0.2102

		1369		0.2095

		1368		0.2089

		1367		0.2083

		1366		0.2078

		1365		0.2074

		1364		0.2071

		1363		0.2068

		1362		0.2066

		1361		0.2065

		1360		0.2064

		1359		0.2063

		1358		0.2062

		1357		0.2062

		1356		0.2061

		1355		0.2061

		1354		0.206

		1353		0.206

		1352		0.2059

		1351		0.2059

		1350		0.2058

		1349		0.2056

		1348		0.2055

		1347		0.2054

		1346		0.2053

		1345		0.2052

		1344		0.2051

		1343		0.2051

		1342		0.205

		1341		0.2049

		1340		0.2049

		1339		0.2049

		1338		0.2049

		1337		0.2049

		1336		0.2049

		1335		0.205

		1334		0.205

		1333		0.2051

		1332		0.2052

		1331		0.2053

		1330		0.2054

		1329		0.2055

		1328		0.2056

		1327		0.2057

		1326		0.2058

		1325		0.206

		1324		0.2061

		1323		0.2063

		1322		0.2064

		1321		0.2066

		1320		0.2068

		1319		0.207

		1318		0.2072

		1317		0.2074

		1316		0.2076

		1315		0.2079

		1314		0.2081

		1313		0.2084

		1312		0.2087

		1311		0.209

		1310		0.2092

		1309		0.2095

		1308		0.2099

		1307		0.2102

		1306		0.2105

		1305		0.2108

		1304		0.2111

		1303		0.2113

		1302		0.2116

		1301		0.2119

		1300		0.2122

		1299		0.2125

		1298		0.2127

		1297		0.213

		1296		0.2132

		1295		0.2134

		1294		0.2136

		1293		0.2138

		1292		0.214

		1291		0.2142

		1290		0.2144

		1289		0.2146

		1288		0.2147

		1287		0.2149

		1286		0.2151

		1285		0.2152

		1284		0.2154

		1283		0.2156

		1282		0.2158

		1281		0.216

		1280		0.2163

		1279		0.2165

		1278		0.2168

		1277		0.2171

		1276		0.2174

		1275		0.2177

		1274		0.2181

		1273		0.2185

		1272		0.219

		1271		0.2195

		1270		0.22

		1269		0.2206

		1268		0.2212

		1267		0.2218

		1266		0.2225

		1265		0.2232

		1264		0.2239

		1263		0.2247

		1262		0.2256

		1261		0.2264

		1260		0.2273

		1259		0.2283

		1258		0.2293

		1257		0.2303

		1256		0.2313

		1255		0.2324

		1254		0.2336

		1253		0.2348

		1252		0.236

		1251		0.2373

		1250		0.2386

		1249		0.24

		1248		0.2415

		1247		0.243

		1246		0.2446

		1245		0.2463

		1244		0.2481

		1243		0.25

		1242		0.252

		1241		0.2541

		1240		0.2564

		1239		0.2587

		1238		0.2613

		1237		0.264

		1236		0.2668

		1235		0.2698

		1234		0.273

		1233		0.2763

		1232		0.2797

		1231		0.2833

		1230		0.2871

		1229		0.2909

		1228		0.2948

		1227		0.2988

		1226		0.3028

		1225		0.3068

		1224		0.3108

		1223		0.3147

		1222		0.3184

		1221		0.322

		1220		0.3254

		1219		0.3285

		1218		0.3314

		1217		0.3339

		1216		0.3362

		1215		0.3381

		1214		0.3396

		1213		0.3407

		1212		0.3415

		1211		0.342

		1210		0.342

		1209		0.3418

		1208		0.3413

		1207		0.3404

		1206		0.3394

		1205		0.3381

		1204		0.3367

		1203		0.3351

		1202		0.3334

		1201		0.3316

		1200		0.3298

		1199		0.3279

		1198		0.326

		1197		0.3241

		1196		0.3222

		1195		0.3204

		1194		0.3185

		1193		0.3167

		1192		0.3149

		1191		0.313

		1190		0.3112

		1189		0.3094

		1188		0.3076

		1187		0.3057

		1186		0.3038

		1185		0.3019

		1184		0.2999

		1183		0.298

		1182		0.296

		1181		0.294

		1180		0.292

		1179		0.29

		1178		0.288

		1177		0.2861

		1176		0.2841

		1175		0.2822

		1174		0.2803

		1173		0.2784

		1172		0.2766

		1171		0.2748

		1170		0.273

		1169		0.2713

		1168		0.2695

		1167		0.2678

		1166		0.2662

		1165		0.2645

		1164		0.2628

		1163		0.2612

		1162		0.2596

		1161		0.258

		1160		0.2563

		1159		0.2547

		1158		0.2531

		1157		0.2515

		1156		0.25

		1155		0.2484

		1154		0.2469

		1153		0.2454

		1152		0.2439

		1151		0.2425

		1150		0.241

		1149		0.2396

		1148		0.2382

		1147		0.2369

		1146		0.2355

		1145		0.2342

		1144		0.2329

		1143		0.2317

		1142		0.2305

		1141		0.2294

		1140		0.2283

		1139		0.2273

		1138		0.2263

		1137		0.2254

		1136		0.2245

		1135		0.2238

		1134		0.223

		1133		0.2224

		1132		0.2218

		1131		0.2213

		1130		0.2209

		1129		0.2206

		1128		0.2203

		1127		0.22

		1126		0.2198

		1125		0.2197

		1124		0.2196

		1123		0.2195

		1122		0.2195

		1121		0.2195

		1120		0.2195

		1119		0.2195

		1118		0.2195

		1117		0.2196

		1116		0.2196

		1115		0.2196

		1114		0.2197

		1113		0.2198

		1112		0.2198

		1111		0.2199

		1110		0.22

		1109		0.22

		1108		0.2201

		1107		0.2202

		1106		0.2203

		1105		0.2204

		1104		0.2204

		1103		0.2206

		1102		0.2207

		1101		0.2208

		1100		0.2209

		1099		0.2211

		1098		0.2212

		1097		0.2214

		1096		0.2216

		1095		0.2217

		1094		0.2219

		1093		0.2221

		1092		0.2223

		1091		0.2225

		1090		0.2228

		1089		0.223

		1088		0.2232

		1087		0.2234

		1086		0.2237

		1085		0.2239

		1084		0.2242

		1083		0.2244

		1082		0.2246

		1081		0.2249

		1080		0.2251

		1079		0.2254

		1078		0.2256

		1077		0.2259

		1076		0.2261

		1075		0.2263

		1074		0.2266

		1073		0.2268

		1072		0.2271

		1071		0.2273

		1070		0.2276

		1069		0.2278

		1068		0.2281

		1067		0.2284

		1066		0.2286

		1065		0.2289

		1064		0.2292

		1063		0.2295

		1062		0.2298

		1061		0.2301

		1060		0.2304

		1059		0.2307

		1058		0.231

		1057		0.2313

		1056		0.2317

		1055		0.232

		1054		0.2323

		1053		0.2327

		1052		0.233

		1051		0.2333

		1050		0.2336

		1049		0.2339

		1048		0.2342

		1047		0.2345

		1046		0.2348

		1045		0.235

		1044		0.2353

		1043		0.2355

		1042		0.2357

		1041		0.2359

		1040		0.236

		1039		0.2361

		1038		0.2362

		1037		0.2363

		1036		0.2363

		1035		0.2364

		1034		0.2363

		1033		0.2363

		1032		0.2363

		1031		0.2362

		1030		0.2361

		1029		0.2361

		1028		0.236

		1027		0.2358

		1026		0.2357

		1025		0.2356

		1024		0.2355

		1023		0.2353

		1022		0.2352

		1021		0.235

		1020		0.2348

		1019		0.2347

		1018		0.2345

		1017		0.2343

		1016		0.2341

		1015		0.2339

		1014		0.2336

		1013		0.2334

		1012		0.2331

		1011		0.2329

		1010		0.2326

		1009		0.2323

		1008		0.232

		1007		0.2317

		1006		0.2314

		1005		0.231

		1004		0.2307

		1003		0.2304

		1002		0.23

		1001		0.2297

		1000		0.2293

		999		0.2289

		998		0.2286

		997		0.2282

		996		0.2278

		995		0.2275

		994		0.2271

		993		0.2267

		992		0.2264

		991		0.226

		990		0.2256

		989		0.2252

		988		0.2248

		987		0.2244

		986		0.224

		985		0.2236

		984		0.2232

		983		0.2228

		982		0.2224

		981		0.222

		980		0.2216

		979		0.2212

		978		0.2207

		977		0.2203

		976		0.2199

		975		0.2194

		974		0.219

		973		0.2185

		972		0.218

		971		0.2175

		970		0.2171

		969		0.2166

		968		0.2161

		967		0.2156

		966		0.215

		965		0.2145

		964		0.214

		963		0.2134

		962		0.2128

		961		0.2123

		960		0.2117

		959		0.2112

		958		0.2106

		957		0.2101

		956		0.2096

		955		0.2092

		954		0.2088

		953		0.2084

		952		0.2081

		951		0.2078

		950		0.2077

		949		0.2076

		948		0.2075

		947		0.2076

		946		0.2077

		945		0.208

		944		0.2083

		943		0.2087

		942		0.2092

		941		0.2098

		940		0.2104

		939		0.2111

		938		0.2118

		937		0.2126

		936		0.2134

		935		0.2142

		934		0.215

		933		0.2158

		932		0.2166

		931		0.2173

		930		0.218

		929		0.2187

		928		0.2192

		927		0.2197

		926		0.2201

		925		0.2205

		924		0.2208

		923		0.2209

		922		0.221

		921		0.221

		920		0.221

		919		0.2208

		918		0.2206

		917		0.2204

		916		0.2201

		915		0.2197

		914		0.2193

		913		0.2189

		912		0.2184

		911		0.2179

		910		0.2174

		909		0.2169

		908		0.2164

		907		0.2158

		906		0.2153

		905		0.2148

		904		0.2143

		903		0.2138

		902		0.2133

		901		0.2128

		900		0.2123

		899		0.2118

		898		0.2114

		897		0.211

		896		0.2105

		895		0.2101

		894		0.2097

		893		0.2094

		892		0.209

		891		0.2087

		890		0.2083

		889		0.208

		888		0.2077

		887		0.2075

		886		0.2072

		885		0.207

		884		0.2068

		883		0.2065

		882		0.2064

		881		0.2062

		880		0.206

		879		0.2059

		878		0.2057

		877		0.2056

		876		0.2056

		875		0.2057

		874		0.2059

		873		0.2062

		872		0.2067

		871		0.2073

		870		0.208

		869		0.2089

		868		0.2099

		867		0.211

		866		0.2123

		865		0.2137

		864		0.2152

		863		0.2168

		862		0.2185

		861		0.2204

		860		0.2224

		859		0.2243

		858		0.2261

		857		0.2278

		856		0.2294

		855		0.2308

		854		0.2322

		853		0.2334

		852		0.2345

		851		0.2354

		850		0.2362

		849		0.2369

		848		0.2375

		847		0.2379

		846		0.2383

		845		0.2384

		844		0.2385

		843		0.2384

		842		0.2383

		841		0.2382

		840		0.238

		839		0.2378

		838		0.2375

		837		0.2373

		836		0.2371

		835		0.2369

		834		0.2366

		833		0.2364

		832		0.2361

		831		0.2358

		830		0.2356

		829		0.2353

		828		0.235

		827		0.2348

		826		0.2346

		825		0.2343

		824		0.2341

		823		0.2339

		822		0.2337

		821		0.2334

		820		0.2332

		819		0.233

		818		0.2329

		817		0.2327

		816		0.2325

		815		0.2324

		814		0.2322

		813		0.232

		812		0.2319

		811		0.2317

		810		0.2316

		809		0.2314

		808		0.2313

		807		0.2312

		806		0.2311

		805		0.2311

		804		0.231

		803		0.2309

		802		0.2308

		801		0.2308

		800		0.2307

		799		0.2306

		798		0.2306

		797		0.2306

		796		0.2305

		795		0.2305

		794		0.2305

		793		0.2304

		792		0.2304

		791		0.2304

		790		0.2303

		789		0.2303

		788		0.2303

		787		0.2302

		786		0.2302

		785		0.2302

		784		0.2301

		783		0.2301

		782		0.2301

		781		0.23

		780		0.23

		779		0.2299

		778		0.2299

		777		0.2299

		776		0.2298

		775		0.2298

		774		0.2298

		773		0.2297

		772		0.2297

		771		0.2297

		770		0.2297

		769		0.2296

		768		0.2296

		767		0.2296

		766		0.2296

		765		0.2295

		764		0.2295

		763		0.2294

		762		0.2294

		761		0.2294

		760		0.2293

		759		0.2292

		758		0.2292

		757		0.2291

		756		0.229

		755		0.2289

		754		0.2288

		753		0.2287

		752		0.2286

		751		0.2285

		750		0.2283

		749		0.2282

		748		0.2281

		747		0.228

		746		0.2278

		745		0.2277

		744		0.2275

		743		0.2274

		742		0.2273

		741		0.2271

		740		0.227

		739		0.2268

		738		0.2267

		737		0.2265

		736		0.2263

		735		0.2262

		734		0.226

		733		0.2259

		732		0.2257

		731		0.2256

		730		0.2255

		729		0.2254

		728		0.2253

		727		0.2251

		726		0.225

		725		0.2249

		724		0.2249

		723		0.2248

		722		0.2247

		721		0.2246

		720		0.2246

		719		0.2245

		718		0.2245

		717		0.2244

		716		0.2243

		715		0.2243

		714		0.2242

		713		0.2241

		712		0.224

		711		0.2239

		710		0.2239

		709		0.2238

		708		0.2237

		707		0.2236

		706		0.2235
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		Method Filename:		C:\Program Files (x86)\PerkinElmer\Pyris\data\Anas\21052024\RT54-MWCNT 0.2 (GNP 0.25-MW 0.75).t6d

		Sample ID:		RT54-MWCNT 0.2 (GNP 0.25-MW 0.75)

		Step:		1

		Data		Sample Temperature (°C)		Weight % (%)
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				31.29		100.1584

				31.3		100.1584

				31.31		100.1584

				31.32		100.1584

				31.33		100.1584

				31.34		100.1584

				31.34		100.1584

				31.35		100.1584

				31.36		100.1584

				31.37		100.1628

				31.38		100.1628

				31.39		100.1628

				31.4		100.1628

				31.41		100.1628

				31.42		100.1628

				31.43		100.1628

				31.43		100.1628

				31.44		100.1628

				31.45		100.1628

				31.46		100.1628

				31.47		100.1628

				31.48		100.1628

				31.49		100.1628

				31.5		100.1628

				31.51		100.1628

				31.52		100.1628

				31.53		100.1628

				31.53		100.1628

				31.54		100.1628

				31.55		100.1628

				31.56		100.1672

				31.57		100.1672

				31.58		100.1672

				31.59		100.1672

				31.6		100.1672

				31.61		100.1672

				31.62		100.1672

				31.63		100.1672

				31.64		100.1672

				31.65		100.1672

				31.66		100.1672

				31.67		100.1672

				31.68		100.1672

				31.69		100.1672

				31.7		100.1672

				31.71		100.1672

				31.72		100.1672

				31.72		100.1672

				31.73		100.1672

				31.74		100.1672

				31.75		100.1672

				31.76		100.1672

				31.77		100.1672

				31.78		100.1672

				31.79		100.1672

				31.8		100.1716

				31.81		100.1716

				31.82		100.1716

				31.83		100.1716

				31.84		100.1716

				31.85		100.1716

				31.86		100.1716

				31.87		100.1716

				31.88		100.1716

				31.89		100.1716

				31.9		100.1716

				31.91		100.1716

				31.92		100.1716

				31.93		100.176

				31.94		100.176

				31.95		100.176

				31.96		100.176

				31.97		100.176

				31.98		100.176

				31.99		100.176

				32.01		100.176

				32.02		100.176

				32.03		100.176

				32.04		100.176

				32.05		100.176

				32.06		100.176

				32.07		100.176

				32.08		100.176

				32.09		100.176

				32.1		100.176

				32.11		100.176

				32.12		100.176

				32.13		100.176

				32.14		100.176

				32.15		100.176

				32.16		100.176

				32.17		100.176

				32.18		100.1804

				32.19		100.176

				32.2		100.1804

				32.22		100.176

				32.23		100.176

				32.24		100.176

				32.25		100.176

				32.26		100.176

				32.27		100.176

				32.28		100.176

				32.29		100.1804

				32.3		100.1804

				32.31		100.1804

				32.32		100.1804

				32.33		100.1804

				32.34		100.1804

				32.36		100.1804

				32.37		100.1804

				32.38		100.1804

				32.39		100.1804

				32.4		100.1804

				32.41		100.1804

				32.42		100.1804

				32.43		100.1804

				32.44		100.1804

				32.46		100.1804

				32.47		100.1804

				32.48		100.1848

				32.49		100.1848

				32.5		100.1848

				32.51		100.1848

				32.52		100.1848

				32.53		100.1848

				32.54		100.1848

				32.56		100.1848

				32.57		100.1848

				32.58		100.1848

				32.59		100.1848

				32.6		100.1848

				32.61		100.1848

				32.62		100.1892

				32.64		100.1892

				32.65		100.1892

				32.66		100.1892

				32.67		100.1892

				32.68		100.1892

				32.69		100.1892

				32.7		100.1892

				32.72		100.1892

				32.73		100.1892

				32.74		100.1892

				32.75		100.1892

				32.76		100.1892

				32.77		100.1936

				32.79		100.1936

				32.8		100.1936

				32.81		100.1936

				32.82		100.1936

				32.83		100.1936

				32.84		100.1936

				32.86		100.1936

				32.87		100.1936

				32.88		100.1936

				32.89		100.1936

				32.9		100.1936

				32.92		100.1936

				32.93		100.1936

				32.94		100.1936

				32.95		100.1936

				32.96		100.1936

				32.98		100.1936

				32.99		100.198

				33		100.198

				33.01		100.198

				33.02		100.198

				33.04		100.198

				33.05		100.198

				33.06		100.198

				33.07		100.198

				33.08		100.198

				33.1		100.198

				33.11		100.198

				33.12		100.198

				33.13		100.198

				33.14		100.198

				33.16		100.198

				33.17		100.198

				33.18		100.198

				33.19		100.198

				33.21		100.198

				33.22		100.198

				33.23		100.2024

				33.24		100.2024

				33.25		100.2024

				33.27		100.2024

				33.28		100.2024

				33.29		100.2024

				33.3		100.2024

				33.32		100.2024

				33.33		100.2024

				33.34		100.2024

				33.35		100.2068

				33.37		100.2068

				33.38		100.2068

				33.39		100.2068

				33.4		100.2068

				33.42		100.2068

				33.43		100.2068

				33.44		100.2068

				33.45		100.2068

				33.47		100.2068

				33.48		100.2068

				33.49		100.2068

				33.51		100.2068

				33.52		100.2068

				33.53		100.2112

				33.54		100.2112

				33.56		100.2112

				33.57		100.2112

				33.58		100.2112

				33.59		100.2112

				33.61		100.2112

				33.62		100.2112

				33.63		100.2112

				33.65		100.2112

				33.66		100.2112

				33.67		100.2112

				33.68		100.2112

				33.7		100.2112

				33.71		100.2112

				33.72		100.2112

				33.74		100.2112

				33.75		100.2112

				33.76		100.2112

				33.78		100.2112

				33.79		100.2156

				33.8		100.2156

				33.81		100.2156

				33.83		100.2156

				33.84		100.2156

				33.85		100.2156

				33.87		100.2156

				33.88		100.2156

				33.89		100.2156

				33.91		100.2156

				33.92		100.2156

				33.93		100.2156

				33.95		100.2156

				33.96		100.2156

				33.97		100.2156

				33.99		100.2156

				34		100.2156

				34.01		100.2156

				34.03		100.2156

				34.04		100.2156

				34.05		100.22

				34.07		100.22

				34.08		100.22

				34.09		100.22

				34.11		100.22

				34.12		100.22

				34.13		100.22

				34.15		100.22

				34.16		100.22

				34.17		100.22

				34.19		100.22

				34.2		100.22

				34.21		100.2244

				34.23		100.2244

				34.24		100.2244

				34.25		100.2244

				34.27		100.2244

				34.28		100.2244

				34.29		100.2244

				34.31		100.2244

				34.32		100.2244

				34.34		100.2244

				34.35		100.2244

				34.36		100.2244

				34.38		100.2244

				34.39		100.2244

				34.4		100.2288

				34.42		100.2288

				34.43		100.2288

				34.45		100.2288

				34.46		100.2288

				34.47		100.2288

				34.49		100.2288

				34.5		100.2288

				34.51		100.2288

				34.53		100.2288

				34.54		100.2288

				34.56		100.2332

				34.57		100.2332

				34.58		100.2332

				34.6		100.2332

				34.61		100.2332

				34.63		100.2332

				34.64		100.2332

				34.65		100.2332

				34.67		100.2332

				34.68		100.2332

				34.7		100.2332

				34.71		100.2332

				34.72		100.2332

				34.74		100.2332

				34.75		100.2332

				34.77		100.2332

				34.78		100.2376

				34.79		100.2376

				34.81		100.2376

				34.82		100.2376

				34.84		100.2376

				34.85		100.2376

				34.87		100.2376

				34.88		100.2376

				34.89		100.2376

				34.91		100.242

				34.92		100.2376

				34.94		100.2376

				34.95		100.242

				34.96		100.242

				34.98		100.242

				34.99		100.242

				35.01		100.242

				35.02		100.242

				35.04		100.242

				35.05		100.242

				35.07		100.242

				35.08		100.242

				35.09		100.242

				35.11		100.2464

				35.12		100.242

				35.14		100.2464

				35.15		100.2464

				35.17		100.2464

				35.18		100.2464

				35.2		100.2464

				35.21		100.2464

				35.22		100.2464

				35.24		100.2464

				35.25		100.2464

				35.27		100.2464

				35.28		100.2508

				35.3		100.2508

				35.31		100.2508

				35.33		100.2508

				35.34		100.2508

				35.36		100.2508

				35.37		100.2508

				35.38		100.2508

				35.4		100.2508

				35.41		100.2508

				35.43		100.2508

				35.44		100.2508

				35.46		100.2508

				35.47		100.2508

				35.49		100.2508

				35.5		100.2508

				35.52		100.2508

				35.53		100.2508

				35.55		100.2508

				35.56		100.2508

				35.58		100.2508

				35.59		100.2508

				35.61		100.2508

				35.62		100.2508

				35.64		100.2508

				35.65		100.2508

				35.67		100.2508

				35.68		100.2552

				35.7		100.2552

				35.71		100.2552

				35.73		100.2552

				35.74		100.2552

				35.76		100.2552

				35.77		100.2552

				35.79		100.2552

				35.8		100.2552

				35.82		100.2552

				35.83		100.2552

				35.85		100.2552

				35.86		100.2552

				35.88		100.2552

				35.89		100.2552

				35.91		100.2552

				35.92		100.2552

				35.94		100.2552

				35.95		100.2552

				35.97		100.2552

				35.98		100.2552

				36		100.2596

				36.01		100.2596

				36.03		100.2596

				36.04		100.2596

				36.06		100.2596

				36.07		100.2596

				36.09		100.2596

				36.1		100.2596

				36.12		100.2596

				36.13		100.2596

				36.15		100.2596

				36.16		100.2596

				36.18		100.2596

				36.19		100.2596

				36.21		100.2596

				36.23		100.264

				36.24		100.264

				36.26		100.264

				36.27		100.264

				36.29		100.264

				36.3		100.264

				36.32		100.264

				36.33		100.264

				36.35		100.264

				36.36		100.264

				36.38		100.2684

				36.39		100.2684

				36.41		100.2684

				36.43		100.2684

				36.44		100.2684

				36.46		100.2684

				36.47		100.2684

				36.49		100.2684

				36.5		100.2684

				36.52		100.2684

				36.53		100.2684

				36.55		100.2728

				36.57		100.2728

				36.58		100.2728

				36.6		100.2728

				36.61		100.2728

				36.63		100.2728

				36.64		100.2728

				36.66		100.2728

				36.67		100.2728

				36.69		100.2728

				36.71		100.2728

				36.72		100.2728

				36.74		100.2728

				36.75		100.2728

				36.77		100.2728

				36.78		100.2728

				36.8		100.2728

				36.82		100.2772

				36.83		100.2772

				36.85		100.2772

				36.86		100.2772

				36.88		100.2772

				36.89		100.2772

				36.91		100.2772

				36.93		100.2816

				36.94		100.2816

				36.96		100.2816

				36.97		100.2816

				36.99		100.2816

				37.01		100.2816

				37.02		100.2816

				37.04		100.2816

				37.05		100.286

				37.07		100.286

				37.08		100.286

				37.1		100.286

				37.12		100.286

				37.13		100.286

				37.15		100.286

				37.16		100.286

				37.18		100.286

				37.2		100.286

				37.21		100.286

				37.23		100.2904

				37.24		100.2904

				37.26		100.2904

				37.28		100.2904

				37.29		100.2904

				37.31		100.2904

				37.32		100.2904

				37.34		100.2904

				37.36		100.2904

				37.37		100.2904

				37.39		100.2948

				37.4		100.2948

				37.42		100.2948

				37.44		100.2948

				37.45		100.2948

				37.47		100.2948

				37.49		100.2948

				37.5		100.2948

				37.52		100.2948

				37.53		100.2948

				37.55		100.2948

				37.57		100.2948

				37.58		100.2948

				37.6		100.2992

				37.62		100.2992

				37.63		100.2992

				37.65		100.2992

				37.66		100.2992

				37.68		100.2992

				37.7		100.2992

				37.71		100.2992

				37.73		100.2992

				37.75		100.2992

				37.76		100.2992

				37.78		100.2992

				37.79		100.2992

				37.81		100.3036

				37.83		100.3036

				37.84		100.3036

				37.86		100.3036

				37.88		100.3036

				37.89		100.3036

				37.91		100.3036

				37.93		100.3036

				37.94		100.3036

				37.96		100.3036

				37.97		100.3036

				37.99		100.3036

				38.01		100.3036

				38.02		100.3036

				38.04		100.3079

				38.06		100.3079

				38.07		100.3079

				38.09		100.3079

				38.11		100.3079

				38.12		100.3079

				38.14		100.3079

				38.16		100.3079

				38.17		100.3079

				38.19		100.3079

				38.21		100.3079

				38.22		100.3079

				38.24		100.3079

				38.26		100.3079

				38.27		100.3123

				38.29		100.3123

				38.31		100.3123

				38.32		100.3123

				38.34		100.3123

				38.36		100.3123

				38.37		100.3123

				38.39		100.3123

				38.41		100.3123

				38.42		100.3123

				38.44		100.3123

				38.46		100.3123

				38.47		100.3123

				38.49		100.3123

				38.51		100.3123

				38.52		100.3123

				38.54		100.3123

				38.56		100.3123

				38.57		100.3123

				38.59		100.3123

				38.61		100.3123

				38.62		100.3167

				38.64		100.3167

				38.66		100.3167

				38.67		100.3167

				38.69		100.3167

				38.71		100.3167

				38.72		100.3167

				38.74		100.3167

				38.76		100.3167

				38.77		100.3167

				38.79		100.3167

				38.81		100.3167

				38.82		100.3167

				38.84		100.3167

				38.86		100.3167

				38.88		100.3211

				38.89		100.3211

				38.91		100.3211

				38.93		100.3211

				38.94		100.3211

				38.96		100.3211

				38.98		100.3211

				38.99		100.3211

				39.01		100.3211

				39.03		100.3211

				39.04		100.3211

				39.06		100.3211

				39.08		100.3211

				39.1		100.3211

				39.11		100.3211

				39.13		100.3211

				39.15		100.3255

				39.16		100.3255

				39.18		100.3255

				39.2		100.3255

				39.22		100.3255

				39.23		100.3255

				39.25		100.3255

				39.27		100.3255

				39.28		100.3255

				39.3		100.3255

				39.32		100.3255

				39.33		100.3255

				39.35		100.3255

				39.37		100.3255

				39.39		100.3255

				39.4		100.3255

				39.42		100.3255

				39.44		100.3255

				39.45		100.3255

				39.47		100.3255

				39.49		100.3255

				39.51		100.3255

				39.52		100.3255

				39.54		100.3255

				39.56		100.3255

				39.58		100.3255

				39.59		100.3255

				39.61		100.3255

				39.63		100.3255

				39.64		100.3255

				39.66		100.3255

				39.68		100.3255

				39.7		100.3255

				39.71		100.3255

				39.73		100.3255

				39.75		100.3255

				39.77		100.3255

				39.78		100.3255

				39.8		100.3255

				39.82		100.3255

				39.83		100.3255

				39.85		100.3255

				39.87		100.3255

				39.89		100.3255

				39.9		100.3255

				39.92		100.3299

				39.94		100.3299

				39.96		100.3299

				39.97		100.3299

				39.99		100.3299

				40.01		100.3299

				40.03		100.3299

				40.04		100.3299

				40.06		100.3299

				40.08		100.3299

				40.1		100.3299

				40.11		100.3299

				40.13		100.3299

				40.15		100.3299

				40.17		100.3299

				40.18		100.3299

				40.2		100.3299

				40.22		100.3299

				40.24		100.3299

				40.25		100.3299

				40.27		100.3343

				40.29		100.3343

				40.31		100.3343

				40.32		100.3343

				40.34		100.3343

				40.36		100.3343

				40.38		100.3343

				40.39		100.3343

				40.41		100.3343

				40.43		100.3343

				40.45		100.3343

				40.46		100.3343

				40.48		100.3343

				40.5		100.3343

				40.52		100.3343

				40.53		100.3343

				40.55		100.3343

				40.57		100.3343

				40.59		100.3343

				40.61		100.3343

				40.62		100.3343

				40.64		100.3343

				40.66		100.3343

				40.68		100.3387

				40.69		100.3387

				40.71		100.3387

				40.73		100.3387

				40.75		100.3387

				40.76		100.3387

				40.78		100.3387

				40.8		100.3387

				40.82		100.3387

				40.84		100.3387

				40.85		100.3387

				40.87		100.3387

				40.89		100.3387

				40.91		100.3387

				40.92		100.3387

				40.94		100.3387

				40.96		100.3431

				40.98		100.3431

				41		100.3431

				41.01		100.3431

				41.03		100.3431

				41.05		100.3431

				41.07		100.3431

				41.08		100.3431

				41.1		100.3431

				41.12		100.3431

				41.14		100.3431

				41.16		100.3431

				41.17		100.3431

				41.19		100.3431

				41.21		100.3431

				41.23		100.3475

				41.25		100.3475

				41.26		100.3475

				41.28		100.3475

				41.3		100.3475

				41.32		100.3475

				41.33		100.3475

				41.35		100.3475

				41.37		100.3475

				41.39		100.3475

				41.41		100.3475

				41.42		100.3475

				41.44		100.3475

				41.46		100.3475

				41.48		100.3475

				41.5		100.3475

				41.51		100.3475

				41.53		100.3475

				41.55		100.3519

				41.57		100.3519

				41.59		100.3519

				41.6		100.3519

				41.62		100.3519

				41.64		100.3519

				41.66		100.3519

				41.68		100.3519

				41.69		100.3519

				41.71		100.3519

				41.73		100.3519

				41.75		100.3519

				41.77		100.3519

				41.78		100.3519

				41.8		100.3519

				41.82		100.3519

				41.84		100.3519

				41.86		100.3519

				41.88		100.3519

				41.89		100.3519

				41.91		100.3519

				41.93		100.3519

				41.95		100.3519

				41.97		100.3519

				41.98		100.3519

				42		100.3519

				42.02		100.3563

				42.04		100.3563

				42.06		100.3563

				42.07		100.3563

				42.09		100.3563

				42.11		100.3563

				42.13		100.3563

				42.15		100.3563

				42.17		100.3563

				42.18		100.3563

				42.2		100.3563

				42.22		100.3563

				42.24		100.3563

				42.26		100.3563

				42.27		100.3563

				42.29		100.3563

				42.31		100.3563

				42.33		100.3563

				42.35		100.3563

				42.37		100.3563

				42.38		100.3563

				42.4		100.3607

				42.42		100.3607

				42.44		100.3607

				42.46		100.3607

				42.48		100.3607

				42.49		100.3607

				42.51		100.3607

				42.53		100.3607

				42.55		100.3607

				42.57		100.3607

				42.59		100.3607

				42.6		100.3607

				42.62		100.3607

				42.64		100.3607

				42.66		100.3607

				42.68		100.3607

				42.7		100.3607

				42.71		100.3607

				42.73		100.3607

				42.75		100.3607

				42.77		100.3607

				42.79		100.3607

				42.81		100.3607

				42.82		100.3607

				42.84		100.3607

				42.86		100.3607

				42.88		100.3607

				42.9		100.3607

				42.92		100.3607

				42.94		100.3607

				42.95		100.3607

				42.97		100.3607

				42.99		100.3607

				43.01		100.3607

				43.03		100.3607

				43.05		100.3651

				43.06		100.3651

				43.08		100.3651

				43.1		100.3651

				43.12		100.3651

				43.14		100.3651

				43.16		100.3651

				43.18		100.3651

				43.19		100.3651

				43.21		100.3651

				43.23		100.3651

				43.25		100.3651

				43.27		100.3651

				43.29		100.3651

				43.31		100.3651

				43.32		100.3651

				43.34		100.3651

				43.36		100.3651

				43.38		100.3695

				43.4		100.3695

				43.42		100.3695

				43.43		100.3695

				43.45		100.3695

				43.47		100.3695

				43.49		100.3695

				43.51		100.3695

				43.53		100.3695

				43.55		100.3695

				43.57		100.3695

				43.58		100.3739

				43.6		100.3739

				43.62		100.3739

				43.64		100.3739

				43.66		100.3739

				43.68		100.3739

				43.7		100.3739

				43.71		100.3739

				43.73		100.3739

				43.75		100.3739

				43.77		100.3739

				43.79		100.3783

				43.81		100.3783

				43.83		100.3783

				43.84		100.3783

				43.86		100.3783

				43.88		100.3783

				43.9		100.3783

				43.92		100.3783

				43.94		100.3783

				43.96		100.3783

				43.98		100.3783

				43.99		100.3783

				44.01		100.3783

				44.03		100.3783

				44.05		100.3783

				44.07		100.3783

				44.09		100.3783

				44.11		100.3783

				44.13		100.3783

				44.14		100.3783

				44.16		100.3783

				44.18		100.3783

				44.2		100.3827

				44.22		100.3827

				44.24		100.3827

				44.26		100.3827

				44.28		100.3827

				44.29		100.3783

				44.31		100.3827

				44.33		100.3827

				44.35		100.3827

				44.37		100.3827

				44.39		100.3827

				44.41		100.3827

				44.43		100.3827

				44.44		100.3827

				44.46		100.3827

				44.48		100.3827

				44.5		100.3827

				44.52		100.3827

				44.54		100.3827

				44.56		100.3871

				44.58		100.3871

				44.6		100.3871

				44.61		100.3871

				44.63		100.3871

				44.65		100.3871

				44.67		100.3871

				44.69		100.3871

				44.71		100.3871

				44.73		100.3871

				44.75		100.3871

				44.77		100.3871

				44.78		100.3871

				44.8		100.3871

				44.82		100.3871

				44.84		100.3871

				44.86		100.3871

				44.88		100.3871

				44.9		100.3871

				44.92		100.3871

				44.94		100.3871

				44.95		100.3915

				44.97		100.3871

				44.99		100.3915

				45.01		100.3915

				45.03		100.3915

				45.05		100.3915

				45.07		100.3915

				45.09		100.3915

				45.11		100.3915

				45.13		100.3915

				45.14		100.3915

				45.16		100.3915

				45.18		100.3915

				45.2		100.3915

				45.22		100.3915

				45.24		100.3915

				45.26		100.3915

				45.28		100.3915

				45.3		100.3915

				45.32		100.3915

				45.33		100.3915

				45.35		100.3915

				45.37		100.3915

				45.39		100.3915

				45.41		100.3915

				45.43		100.3915

				45.45		100.3915

				45.47		100.3959

				45.49		100.3959

				45.51		100.3959

				45.53		100.3959

				45.54		100.3959

				45.56		100.3959

				45.58		100.3959

				45.6		100.3959

				45.62		100.3959

				45.64		100.3959

				45.66		100.3959

				45.68		100.3959

				45.7		100.3959

				45.72		100.3959

				45.74		100.3959

				45.75		100.3959

				45.77		100.3959

				45.79		100.3959

				45.81		100.3959

				45.83		100.3959

				45.85		100.3959

				45.87		100.3959

				45.89		100.4003

				45.91		100.4003

				45.93		100.4003

				45.95		100.4003

				45.97		100.4003

				45.98		100.4003

				46		100.4003

				46.02		100.4003

				46.04		100.4003

				46.06		100.4003

				46.08		100.4003

				46.1		100.4003

				46.12		100.4003

				46.14		100.4047

				46.16		100.4047

				46.18		100.4047

				46.2		100.4047

				46.22		100.4047

				46.23		100.4047

				46.25		100.4047

				46.27		100.4047

				46.29		100.4047

				46.31		100.4047

				46.33		100.4091

				46.35		100.4091

				46.37		100.4091

				46.39		100.4091

				46.41		100.4091

				46.43		100.4091

				46.45		100.4091

				46.47		100.4091

				46.48		100.4091

				46.5		100.4091

				46.52		100.4091

				46.54		100.4091

				46.56		100.4091

				46.58		100.4091

				46.6		100.4135

				46.62		100.4135

				46.64		100.4135

				46.66		100.4135

				46.68		100.4135

				46.7		100.4135

				46.72		100.4135

				46.74		100.4135

				46.75		100.4135

				46.77		100.4135

				46.79		100.4135

				46.81		100.4135

				46.83		100.4135

				46.85		100.4135

				46.87		100.4135

				46.89		100.4135

				46.91		100.4135

				46.93		100.4135

				46.95		100.4135

				46.97		100.4135

				46.99		100.4135

				47.01		100.4135

				47.03		100.4135

				47.04		100.4135

				47.06		100.4135

				47.08		100.4135

				47.1		100.4135

				47.12		100.4135

				47.14		100.4179

				47.16		100.4179

				47.18		100.4179

				47.2		100.4179

				47.22		100.4179

				47.24		100.4179

				47.26		100.4179

				47.28		100.4179

				47.3		100.4179

				47.32		100.4179

				47.34		100.4179

				47.36		100.4179

				47.37		100.4179

				47.39		100.4179

				47.41		100.4179

				47.43		100.4179

				47.45		100.4179

				47.47		100.4179

				47.49		100.4179

				47.51		100.4179

				47.53		100.4179

				47.55		100.4179

				47.57		100.4179

				47.59		100.4179

				47.61		100.4179

				47.63		100.4179

				47.65		100.4179

				47.67		100.4179

				47.69		100.4179

				47.71		100.4179

				47.72		100.4179

				47.74		100.4179

				47.76		100.4179

				47.78		100.4179

				47.8		100.4179

				47.82		100.4179

				47.84		100.4179

				47.86		100.4179

				47.88		100.4179

				47.9		100.4179

				47.92		100.4179

				47.94		100.4179

				47.96		100.4179

				47.98		100.4223

				48		100.4223

				48.02		100.4179

				48.04		100.4179

				48.06		100.4223

				48.08		100.4223

				48.1		100.4223

				48.12		100.4223

				48.13		100.4223

				48.15		100.4223

				48.17		100.4223

				48.19		100.4179

				48.21		100.4223

				48.23		100.4179

				48.25		100.4223

				48.27		100.4179

				48.29		100.4179

				48.31		100.4223

				48.33		100.4223

				48.35		100.4223

				48.37		100.4223

				48.39		100.4223

				48.41		100.4223

				48.43		100.4223

				48.45		100.4223

				48.47		100.4223

				48.49		100.4223

				48.51		100.4223

				48.53		100.4223

				48.55		100.4223

				48.57		100.4223

				48.59		100.4223

				48.6		100.4223

				48.62		100.4223

				48.64		100.4223

				48.66		100.4223

				48.68		100.4223

				48.7		100.4223

				48.72		100.4223

				48.74		100.4223

				48.76		100.4223

				48.78		100.4223

				48.8		100.4223

				48.82		100.4223

				48.84		100.4223

				48.86		100.4267

				48.88		100.4267

				48.9		100.4267

				48.92		100.4267

				48.94		100.4267

				48.96		100.4267

				48.98		100.4267

				49		100.4267

				49.02		100.4267

				49.04		100.4267

				49.06		100.4267

				49.08		100.4267

				49.1		100.4267

				49.12		100.4267

				49.14		100.4267

				49.16		100.4267

				49.18		100.4267

				49.2		100.4267

				49.21		100.4267

				49.23		100.4267

				49.25		100.4267

				49.27		100.4267

				49.29		100.4267

				49.31		100.4311

				49.33		100.4311

				49.35		100.4311

				49.37		100.4311

				49.39		100.4311

				49.41		100.4311

				49.43		100.4311

				49.45		100.4311

				49.47		100.4311

				49.49		100.4311

				49.51		100.4311

				49.53		100.4311

				49.55		100.4311

				49.57		100.4311

				49.59		100.4311

				49.61		100.4311

				49.63		100.4311

				49.65		100.4311

				49.67		100.4311

				49.69		100.4311

				49.71		100.4311

				49.73		100.4311

				49.75		100.4311

				49.77		100.4311

				49.79		100.4355

				49.81		100.4355

				49.83		100.4355

				49.85		100.4355

				49.87		100.4355

				49.89		100.4355

				49.91		100.4355

				49.93		100.4355

				49.95		100.4355

				49.97		100.4355

				49.99		100.4355

				50.01		100.4355

				50.03		100.4355

				50.05		100.4355

				50.07		100.4355

				50.08		100.4355

				50.1		100.4355

				50.12		100.4355

				50.14		100.4355

				50.16		100.4355

				50.18		100.4355

				50.2		100.4355

				50.22		100.4355

				50.24		100.4355

				50.26		100.4355

				50.28		100.4355

				50.3		100.4355

				50.32		100.4355

				50.34		100.4355

				50.36		100.4355

				50.38		100.4355

				50.4		100.4355

				50.42		100.4355

				50.44		100.4355

				50.46		100.4355

				50.48		100.4355

				50.5		100.4355

				50.52		100.4355

				50.54		100.4355

				50.56		100.4355

				50.58		100.4355

				50.6		100.4355

				50.62		100.4355

				50.64		100.4355

				50.66		100.4355

				50.68		100.4399

				50.7		100.4399

				50.72		100.4399

				50.74		100.4399

				50.76		100.4399

				50.78		100.4399

				50.8		100.4399

				50.82		100.4399

				50.84		100.4399

				50.86		100.4399

				50.88		100.4399

				50.9		100.4399

				50.92		100.4399

				50.94		100.4399

				50.96		100.4399

				50.98		100.4399

				51		100.4399

				51.02		100.4399

				51.04		100.4399

				51.06		100.4399

				51.08		100.4399

				51.1		100.4399

				51.12		100.4399

				51.14		100.4443

				51.16		100.4443

				51.18		100.4443

				51.2		100.4443

				51.22		100.4443

				51.24		100.4443

				51.26		100.4443

				51.28		100.4443

				51.3		100.4443

				51.32		100.4443

				51.34		100.4487

				51.36		100.4487

				51.38		100.4487

				51.4		100.4487

				51.42		100.4487

				51.44		100.4487

				51.46		100.4487

				51.48		100.4487

				51.5		100.4487

				51.52		100.4487

				51.54		100.4487

				51.56		100.4487

				51.58		100.4487

				51.6		100.4487

				51.62		100.4487

				51.64		100.4531

				51.66		100.4531

				51.68		100.4531

				51.7		100.4531

				51.72		100.4531

				51.74		100.4531

				51.76		100.4531

				51.78		100.4531

				51.8		100.4531

				51.82		100.4531

				51.84		100.4531

				51.86		100.4531

				51.88		100.4531

				51.9		100.4531

				51.92		100.4531

				51.94		100.4531

				51.96		100.4531

				51.98		100.4531

				52		100.4531

				52.02		100.4531

				52.04		100.4531

				52.06		100.4575

				52.08		100.4531

				52.1		100.4575

				52.12		100.4575

				52.14		100.4575

				52.16		100.4575

				52.18		100.4575

				52.2		100.4575

				52.22		100.4575

				52.24		100.4575

				52.26		100.4575

				52.28		100.4575

				52.3		100.4619

				52.32		100.4619

				52.34		100.4619

				52.36		100.4619

				52.38		100.4619

				52.4		100.4619

				52.42		100.4619

				52.44		100.4619

				52.46		100.4663

				52.48		100.4663

				52.5		100.4663

				52.52		100.4663

				52.54		100.4663

				52.56		100.4663

				52.58		100.4663

				52.6		100.4663

				52.62		100.4663

				52.64		100.4663

				52.66		100.4663

				52.68		100.4663

				52.7		100.4663

				52.72		100.4707

				52.74		100.4707

				52.76		100.4707

				52.78		100.4707

				52.8		100.4707

				52.82		100.4707

				52.84		100.4707

				52.86		100.4707

				52.88		100.4707

				52.9		100.4707

				52.92		100.4707

				52.94		100.4707

				52.96		100.4707

				52.98		100.4751

				53		100.4751

				53.02		100.4751

				53.04		100.4751

				53.06		100.4751

				53.08		100.4751

				53.1		100.4751

				53.13		100.4751

				53.15		100.4751

				53.17		100.4751

				53.19		100.4751

				53.21		100.4751

				53.23		100.4751

				53.25		100.4751

				53.27		100.4751

				53.29		100.4751

				53.31		100.4751

				53.33		100.4751

				53.35		100.4751

				53.37		100.4751

				53.39		100.4751

				53.41		100.4751

				53.43		100.4751

				53.45		100.4751

				53.47		100.4751

				53.49		100.4795

				53.51		100.4795

				53.53		100.4795

				53.55		100.4795

				53.57		100.4795

				53.59		100.4795

				53.61		100.4795

				53.63		100.4795

				53.65		100.4795

				53.67		100.4795

				53.69		100.4795

				53.71		100.4795

				53.73		100.4795

				53.75		100.4795

				53.77		100.4795

				53.79		100.4795

				53.81		100.4795

				53.83		100.4795

				53.85		100.4795

				53.87		100.4795

				53.89		100.4795

				53.91		100.4795

				53.93		100.4795

				53.95		100.4795

				53.97		100.4795

				53.99		100.4795

				54.01		100.4795

				54.03		100.4795

				54.05		100.4795

				54.08		100.4795

				54.1		100.4795

				54.12		100.4795

				54.14		100.4795

				54.16		100.4795

				54.18		100.4795

				54.2		100.4795

				54.22		100.4795

				54.24		100.4795

				54.26		100.4795

				54.28		100.4795

				54.3		100.4795

				54.32		100.4795

				54.34		100.4795

				54.36		100.4839

				54.38		100.4839

				54.4		100.4839

				54.42		100.4839

				54.44		100.4839

				54.46		100.4839

				54.48		100.4839

				54.5		100.4839

				54.52		100.4839

				54.54		100.4839

				54.56		100.4839

				54.58		100.4839

				54.6		100.4839

				54.62		100.4839

				54.64		100.4839

				54.66		100.4839

				54.68		100.4839

				54.7		100.4839

				54.72		100.4839

				54.74		100.4883

				54.77		100.4839

				54.79		100.4839

				54.81		100.4883

				54.83		100.4883

				54.85		100.4883

				54.87		100.4883

				54.89		100.4883

				54.91		100.4883

				54.93		100.4883

				54.95		100.4883

				54.97		100.4883

				54.99		100.4883

				55.01		100.4883

				55.03		100.4883

				55.05		100.4883

				55.07		100.4883

				55.09		100.4883

				55.11		100.4883

				55.13		100.4883

				55.15		100.4883

				55.17		100.4883

				55.19		100.4883

				55.21		100.4883

				55.23		100.4883

				55.25		100.4883

				55.27		100.4883

				55.29		100.4883

				55.31		100.4883

				55.33		100.4883

				55.36		100.4883

				55.38		100.4883

				55.4		100.4883

				55.42		100.4883

				55.44		100.4883

				55.46		100.4883

				55.48		100.4883

				55.5		100.4883

				55.52		100.4883

				55.54		100.4883

				55.56		100.4883

				55.58		100.4883

				55.6		100.4883

				55.62		100.4883

				55.64		100.4883

				55.66		100.4883

				55.68		100.4883

				55.7		100.4883

				55.72		100.4883

				55.74		100.4883

				55.76		100.4883

				55.78		100.4883

				55.8		100.4927

				55.82		100.4927

				55.84		100.4927

				55.86		100.4927

				55.89		100.4927

				55.91		100.4927

				55.93		100.4927

				55.95		100.4927

				55.97		100.4927

				55.99		100.4927

				56.01		100.4927

				56.03		100.4927

				56.05		100.4927

				56.07		100.4927

				56.09		100.4971

				56.11		100.4971

				56.13		100.4971

				56.15		100.4971

				56.17		100.4971

				56.19		100.4971

				56.21		100.4971

				56.23		100.4971

				56.25		100.4971

				56.27		100.4971

				56.29		100.4971

				56.31		100.4971

				56.33		100.4971

				56.35		100.4971

				56.37		100.4971

				56.4		100.4971

				56.42		100.4971

				56.44		100.4971

				56.46		100.4971

				56.48		100.4971

				56.5		100.4971

				56.52		100.4971

				56.54		100.4971

				56.56		100.4971

				56.58		100.4971

				56.6		100.4971

				56.62		100.4971

				56.64		100.4971

				56.66		100.5015

				56.68		100.4971

				56.7		100.5015

				56.72		100.5015

				56.74		100.5015

				56.76		100.5015

				56.78		100.5015

				56.8		100.5015

				56.82		100.5015

				56.84		100.5015

				56.87		100.5015

				56.89		100.5015

				56.91		100.5015

				56.93		100.5015

				56.95		100.5015

				56.97		100.5015

				56.99		100.5015

				57.01		100.5015

				57.03		100.5015

				57.05		100.5015

				57.07		100.5015

				57.09		100.5015

				57.11		100.5015

				57.13		100.5015

				57.15		100.5015

				57.17		100.5015

				57.19		100.5015

				57.21		100.5015

				57.23		100.5015

				57.25		100.5015

				57.27		100.5015

				57.3		100.5015

				57.32		100.5015

				57.34		100.5015

				57.36		100.5015

				57.38		100.5015

				57.4		100.5015

				57.42		100.5015

				57.44		100.5015

				57.46		100.5015

				57.48		100.5015

				57.5		100.5015

				57.52		100.5015

				57.54		100.5015

				57.56		100.5059

				57.58		100.5059

				57.6		100.5059

				57.62		100.5059

				57.64		100.5059

				57.66		100.5059

				57.68		100.5059

				57.71		100.5059

				57.73		100.5059

				57.75		100.5059

				57.77		100.5059

				57.79		100.5059

				57.81		100.5059

				57.83		100.5059

				57.85		100.5059

				57.87		100.5059

				57.89		100.5059

				57.91		100.5059

				57.93		100.5059

				57.95		100.5059

				57.97		100.5059

				57.99		100.5059

				58.01		100.5059

				58.03		100.5059

				58.05		100.5059

				58.07		100.5059

				58.1		100.5059

				58.12		100.5059

				58.14		100.5059

				58.16		100.5059

				58.18		100.5059

				58.2		100.5059

				58.22		100.5059

				58.24		100.5059

				58.26		100.5059

				58.28		100.5059

				58.3		100.5059

				58.32		100.5059

				58.34		100.5059

				58.36		100.5059

				58.38		100.5059

				58.4		100.5059

				58.42		100.5059

				58.44		100.5059

				58.47		100.5059

				58.49		100.5059

				58.51		100.5103

				58.53		100.5103

				58.55		100.5103

				58.57		100.5103

				58.59		100.5103

				58.61		100.5103

				58.63		100.5103

				58.65		100.5103

				58.67		100.5103

				58.69		100.5103

				58.71		100.5103

				58.73		100.5103

				58.75		100.5103

				58.77		100.5103

				58.79		100.5103

				58.82		100.5103

				58.84		100.5103

				58.86		100.5103

				58.88		100.5103

				58.9		100.5103

				58.92		100.5103

				58.94		100.5103

				58.96		100.5103

				58.98		100.5103

				59		100.5103

				59.02		100.5103

				59.04		100.5103

				59.06		100.5103

				59.08		100.5103

				59.1		100.5103

				59.12		100.5147

				59.14		100.5147

				59.17		100.5147

				59.19		100.5147

				59.21		100.5147

				59.23		100.5147

				59.25		100.5147

				59.27		100.5147

				59.29		100.5147

				59.31		100.5147

				59.33		100.5147

				59.35		100.5147

				59.37		100.5191

				59.39		100.5191

				59.41		100.5191

				59.43		100.5191

				59.45		100.5191

				59.47		100.5191

				59.49		100.5191

				59.52		100.5191

				59.54		100.5191

				59.56		100.5235

				59.58		100.5235

				59.6		100.5235

				59.62		100.5235

				59.64		100.5235

				59.66		100.5235

				59.68		100.5235

				59.7		100.5235

				59.72		100.5235

				59.74		100.5235

				59.76		100.5235

				59.78		100.5235

				59.8		100.5235

				59.82		100.5279

				59.84		100.5279

				59.87		100.5279

				59.89		100.5279

				59.91		100.5279

				59.93		100.5279

				59.95		100.5279

				59.97		100.5323

				59.99		100.5323

				60.01		100.5323

				60.03		100.5323

				60.05		100.5323

				60.07		100.5323

				60.09		100.5323

				60.11		100.5323

				60.13		100.5323

				60.15		100.5323

				60.17		100.5367

				60.19		100.5367

				60.22		100.5367

				60.24		100.5367

				60.26		100.5367

				60.28		100.5367

				60.3		100.5367

				60.32		100.5367

				60.34		100.5367

				60.36		100.5411

				60.38		100.5411

				60.4		100.5411

				60.42		100.5411

				60.44		100.5411

				60.46		100.5411

				60.48		100.5411

				60.5		100.5411

				60.52		100.5411

				60.54		100.5411

				60.57		100.5411

				60.59		100.5455

				60.61		100.5455

				60.63		100.5455

				60.65		100.5455

				60.67		100.5455

				60.69		100.5455

				60.71		100.5455

				60.73		100.5455

				60.75		100.5455

				60.77		100.5455

				60.79		100.5455

				60.81		100.5455

				60.83		100.5499

				60.85		100.5499

				60.87		100.5499

				60.89		100.5499

				60.92		100.5499

				60.94		100.5499

				60.96		100.5499

				60.98		100.5499

				61		100.5499

				61.02		100.5499

				61.04		100.5499

				61.06		100.5499

				61.08		100.5499

				61.1		100.5499

				61.12		100.5499

				61.14		100.5499

				61.16		100.5499

				61.18		100.5499

				61.2		100.5499

				61.22		100.5499

				61.24		100.5499

				61.26		100.5499

				61.29		100.5499

				61.31		100.5499

				61.33		100.5499

				61.35		100.5499

				61.37		100.5543

				61.39		100.5543

				61.41		100.5543

				61.43		100.5543

				61.45		100.5543

				61.47		100.5543

				61.49		100.5543

				61.51		100.5543

				61.53		100.5543

				61.55		100.5543

				61.57		100.5543

				61.59		100.5543

				61.61		100.5543

				61.63		100.5543

				61.65		100.5543

				61.68		100.5543

				61.7		100.5543

				61.72		100.5543

				61.74		100.5543

				61.76		100.5543

				61.78		100.5543

				61.8		100.5543

				61.82		100.5543

				61.84		100.5543

				61.86		100.5543

				61.88		100.5543

				61.9		100.5543

				61.92		100.5587

				61.94		100.5543

				61.96		100.5543

				61.98		100.5543

				62		100.5543

				62.02		100.5543

				62.04		100.5543

				62.06		100.5543

				62.09		100.5587

				62.11		100.5587

				62.13		100.5587

				62.15		100.5587

				62.17		100.5587

				62.19		100.5587

				62.21		100.5587

				62.23		100.5587

				62.25		100.5587

				62.27		100.5587

				62.29		100.5587

				62.31		100.5587

				62.33		100.5587

				62.35		100.5587

				62.37		100.5587

				62.39		100.5587

				62.41		100.5587

				62.43		100.5587

				62.45		100.5587

				62.48		100.5587

				62.5		100.5587

				62.52		100.5587

				62.54		100.5587

				62.56		100.5587

				62.58		100.5587

				62.6		100.5587

				62.62		100.5587

				62.64		100.5587

				62.66		100.5587

				62.68		100.5631

				62.7		100.5631

				62.72		100.5631

				62.74		100.5631

				62.76		100.5631

				62.78		100.5631

				62.8		100.5631

				62.82		100.5631

				62.84		100.5631

				62.86		100.5631

				62.89		100.5631

				62.91		100.5631

				62.93		100.5631

				62.95		100.5631

				62.97		100.5631

				62.99		100.5631

				63.01		100.5631

				63.03		100.5631

				63.05		100.5631

				63.07		100.5631

				63.09		100.5631

				63.11		100.5631

				63.13		100.5631

				63.15		100.5631

				63.17		100.5631

				63.19		100.5631

				63.21		100.5631

				63.23		100.5631

				63.25		100.5675

				63.27		100.5631

				63.29		100.5675

				63.32		100.5675

				63.34		100.5675

				63.36		100.5675

				63.38		100.5675

				63.4		100.5675

				63.42		100.5675

				63.44		100.5675

				63.46		100.5675

				63.48		100.5675

				63.5		100.5675

				63.52		100.5675

				63.54		100.5675

				63.56		100.5675

				63.58		100.5675

				63.6		100.5675

				63.62		100.5675

				63.64		100.5675

				63.66		100.5675

				63.68		100.5675

				63.7		100.5675

				63.72		100.5675

				63.75		100.5675

				63.77		100.5675

				63.79		100.5675

				63.81		100.5675

				63.83		100.5675

				63.85		100.5675

				63.87		100.5675

				63.89		100.5675

				63.91		100.5675

				63.93		100.5675

				63.95		100.5675

				63.97		100.5675

				63.99		100.5675

				64.01		100.5675

				64.03		100.5675

				64.05		100.5675

				64.07		100.5675

				64.09		100.5675

				64.11		100.5675

				64.13		100.5675

				64.16		100.5675

				64.18		100.5675

				64.2		100.5675

				64.22		100.5675

				64.24		100.5675

				64.26		100.5675

				64.28		100.5675

				64.3		100.5675

				64.32		100.5675

				64.34		100.5675

				64.36		100.5719

				64.38		100.5719

				64.4		100.5719

				64.42		100.5719

				64.44		100.5719

				64.46		100.5719

				64.48		100.5719

				64.5		100.5719

				64.52		100.5719

				64.54		100.5719

				64.57		100.5719

				64.59		100.5719

				64.61		100.5719

				64.63		100.5719

				64.65		100.5719

				64.67		100.5719

				64.69		100.5719

				64.71		100.5719

				64.73		100.5719

				64.75		100.5719

				64.77		100.5719

				64.79		100.5719

				64.81		100.5719

				64.83		100.5719

				64.85		100.5719

				64.87		100.5719

				64.89		100.5719

				64.91		100.5719

				64.93		100.5719

				64.96		100.5719

				64.98		100.5719

				65		100.5719

				65.02		100.5719

				65.04		100.5719

				65.06		100.5719

				65.08		100.5719

				65.1		100.5719

				65.12		100.5719

				65.14		100.5719

				65.16		100.5719

				65.18		100.5719

				65.2		100.5719

				65.22		100.5719

				65.24		100.5719

				65.26		100.5719

				65.28		100.5719

				65.3		100.5719

				65.32		100.5719

				65.35		100.5719

				65.37		100.5719

				65.39		100.5719

				65.41		100.5763

				65.43		100.5763

				65.45		100.5763

				65.47		100.5763

				65.49		100.5763

				65.51		100.5763

				65.53		100.5763

				65.55		100.5763

				65.57		100.5763

				65.59		100.5763

				65.61		100.5763

				65.63		100.5763

				65.65		100.5763

				65.67		100.5763

				65.69		100.5763

				65.72		100.5763

				65.74		100.5763

				65.76		100.5807

				65.78		100.5807

				65.8		100.5807

				65.82		100.5807

				65.84		100.5807

				65.86		100.5807

				65.88		100.5807

				65.9		100.5807

				65.92		100.5807

				65.94		100.5807

				65.96		100.5807

				65.98		100.5807

				66		100.5807

				66.02		100.5807

				66.04		100.5807

				66.07		100.5807

				66.09		100.5851

				66.11		100.5851

				66.13		100.5851

				66.15		100.5851

				66.17		100.5851

				66.19		100.5851

				66.21		100.5851

				66.23		100.5851

				66.25		100.5851

				66.27		100.5851

				66.29		100.5851

				66.31		100.5851

				66.33		100.5851

				66.35		100.5851

				66.37		100.5851

				66.39		100.5851

				66.42		100.5851

				66.44		100.5851

				66.46		100.5895

				66.48		100.5895

				66.5		100.5895

				66.52		100.5895

				66.54		100.5895

				66.56		100.5895

				66.58		100.5895

				66.6		100.5895

				66.62		100.5895

				66.64		100.5895

				66.66		100.5895

				66.68		100.5895

				66.7		100.5895

				66.72		100.5895

				66.75		100.5895

				66.77		100.5895

				66.79		100.5895

				66.81		100.5895

				66.83		100.5895

				66.85		100.5895

				66.87		100.5895

				66.89		100.5895

				66.91		100.5895

				66.93		100.5895

				66.95		100.5895

				66.97		100.5895

				66.99		100.5939

				67.01		100.5939

				67.03		100.5895

				67.06		100.5939

				67.08		100.5895

				67.1		100.5895

				67.12		100.5895

				67.14		100.5895

				67.16		100.5895

				67.18		100.5895

				67.2		100.5895

				67.22		100.5895

				67.24		100.5939

				67.26		100.5939

				67.28		100.5939

				67.3		100.5939

				67.32		100.5939

				67.34		100.5939

				67.37		100.5939

				67.39		100.5939

				67.41		100.5939

				67.43		100.5939

				67.45		100.5939

				67.47		100.5939

				67.49		100.5939

				67.51		100.5939

				67.53		100.5939

				67.55		100.5983

				67.57		100.5983

				67.59		100.5983

				67.61		100.5983

				67.63		100.5983

				67.65		100.5983

				67.68		100.5983

				67.7		100.5983

				67.72		100.5983

				67.74		100.5983

				67.76		100.5983

				67.78		100.5983

				67.8		100.5983

				67.82		100.5983

				67.84		100.5983

				67.86		100.5983

				67.88		100.5983

				67.9		100.5983

				67.92		100.5983

				67.94		100.5983

				67.97		100.5983

				67.99		100.5983

				68.01		100.5983

				68.03		100.5983

				68.05		100.5983

				68.07		100.5983

				68.09		100.5983

				68.11		100.5983

				68.13		100.5983

				68.15		100.5983

				68.17		100.5983

				68.19		100.5983

				68.21		100.5983

				68.23		100.5983

				68.26		100.5983

				68.28		100.5983

				68.3		100.5983

				68.32		100.5983

				68.34		100.5983

				68.36		100.5983

				68.38		100.5983

				68.4		100.5983

				68.42		100.5983

				68.44		100.5939

				68.46		100.5939

				68.48		100.5939

				68.5		100.5939

				68.53		100.5939

				68.55		100.5939

				68.57		100.5939

				68.59		100.5939

				68.61		100.5939

				68.63		100.5939

				68.65		100.5939

				68.67		100.5939

				68.69		100.5939

				68.71		100.5939

				68.73		100.5939

				68.75		100.5983

				68.77		100.5983

				68.8		100.5983

				68.82		100.5983

				68.84		100.5983

				68.86		100.5983

				68.88		100.5983

				68.9		100.5983

				68.92		100.5983

				68.94		100.5983

				68.96		100.5983

				68.98		100.5983

				69		100.5983

				69.02		100.5983

				69.04		100.5983

				69.07		100.5983

				69.09		100.5983

				69.11		100.5983

				69.13		100.5983

				69.15		100.5983

				69.17		100.5983

				69.19		100.5983

				69.21		100.5983

				69.23		100.6027

				69.25		100.6027

				69.27		100.6027

				69.29		100.6027

				69.31		100.6027

				69.34		100.6027

				69.36		100.6027

				69.38		100.6027

				69.4		100.6027

				69.42		100.6027

				69.44		100.6027

				69.46		100.6027

				69.48		100.6027

				69.5		100.6027

				69.52		100.6027

				69.54		100.6027

				69.56		100.6027

				69.58		100.6027

				69.61		100.6027

				69.63		100.6027

				69.65		100.6027

				69.67		100.6027

				69.69		100.6027

				69.71		100.6027

				69.73		100.6027

				69.75		100.6027

				69.77		100.6027

				69.79		100.6027

				69.81		100.6027

				69.83		100.6027

				69.86		100.6027

				69.88		100.6027

				69.9		100.6027

				69.92		100.6027

				69.94		100.6027

				69.96		100.6027

				69.98		100.6027

				70		100.6027

				70.02		100.6027

				70.04		100.6027

				70.06		100.6027

				70.08		100.6027

				70.11		100.6027

				70.13		100.6027

				70.15		100.6071

				70.17		100.6071

				70.19		100.6071

				70.21		100.6071

				70.23		100.6071

				70.25		100.6071

				70.27		100.6071

				70.29		100.6071

				70.31		100.6071

				70.33		100.6071

				70.36		100.6071

				70.38		100.6071

				70.4		100.6071

				70.42		100.6071

				70.44		100.6071

				70.46		100.6071

				70.48		100.6071

				70.5		100.6071

				70.52		100.6071

				70.54		100.6071

				70.56		100.6071

				70.59		100.6071

				70.61		100.6071

				70.63		100.6071

				70.65		100.6071

				70.67		100.6071

				70.69		100.6071

				70.71		100.6115

				70.73		100.6115

				70.75		100.6115

				70.77		100.6115

				70.79		100.6115

				70.81		100.6115

				70.84		100.6115

				70.86		100.6115

				70.88		100.6115

				70.9		100.6115

				70.92		100.6115

				70.94		100.6115

				70.96		100.6115

				70.98		100.6115

				71		100.6115

				71.02		100.6115

				71.04		100.6115

				71.06		100.6115

				71.09		100.6115

				71.11		100.6115

				71.13		100.6115

				71.15		100.6115

				71.17		100.6115

				71.19		100.6115

				71.21		100.6115

				71.23		100.6115

				71.25		100.6115

				71.27		100.6115

				71.29		100.6115

				71.32		100.6115

				71.34		100.6115

				71.36		100.6115

				71.38		100.6115

				71.4		100.6115

				71.42		100.6159

				71.44		100.6159

				71.46		100.6159

				71.48		100.6159

				71.5		100.6159

				71.52		100.6159

				71.54		100.6159

				71.57		100.6159

				71.59		100.6159

				71.61		100.6159

				71.63		100.6159

				71.65		100.6159

				71.67		100.6159

				71.69		100.6159

				71.71		100.6159

				71.73		100.6159

				71.75		100.6159

				71.77		100.6203

				71.8		100.6203

				71.82		100.6203

				71.84		100.6203

				71.86		100.6203

				71.88		100.6203

				71.9		100.6203

				71.92		100.6203

				71.94		100.6203

				71.96		100.6203

				71.98		100.6203

				72		100.6203

				72.03		100.6203

				72.05		100.6203

				72.07		100.6203

				72.09		100.6247

				72.11		100.6247

				72.13		100.6247

				72.15		100.6247

				72.17		100.6247

				72.19		100.6247

				72.21		100.6247

				72.23		100.6247

				72.26		100.6247

				72.28		100.6247

				72.3		100.6247

				72.32		100.6247

				72.34		100.6247

				72.36		100.6247

				72.38		100.6247

				72.4		100.6247

				72.42		100.6247

				72.44		100.6247

				72.46		100.6247

				72.49		100.6247

				72.51		100.6247

				72.53		100.6247

				72.55		100.6247

				72.57		100.6247

				72.59		100.6247

				72.61		100.6247

				72.63		100.6247

				72.65		100.6247

				72.67		100.6247

				72.69		100.6247

				72.72		100.6247

				72.74		100.6247

				72.76		100.6247

				72.78		100.6247

				72.8		100.6247

				72.82		100.6247

				72.84		100.6247

				72.86		100.6247

				72.88		100.6247

				72.9		100.6247

				72.92		100.6247

				72.95		100.6247

				72.97		100.6247

				72.99		100.6291

				73.01		100.6291

				73.03		100.6247

				73.05		100.6291

				73.07		100.6291

				73.09		100.6291

				73.11		100.6291

				73.13		100.6291

				73.16		100.6291

				73.18		100.6291

				73.2		100.6291

				73.22		100.6291

				73.24		100.6291

				73.26		100.6291

				73.28		100.6291

				73.3		100.6291

				73.32		100.6291

				73.34		100.6291

				73.36		100.6291

				73.39		100.6291

				73.41		100.6291

				73.43		100.6291

				73.45		100.6291

				73.47		100.6291

				73.49		100.6291

				73.51		100.6291

				73.53		100.6291

				73.55		100.6291

				73.57		100.6291

				73.6		100.6291

				73.62		100.6291

				73.64		100.6291

				73.66		100.6291

				73.68		100.6291

				73.7		100.6291

				73.72		100.6291

				73.74		100.6291

				73.76		100.6291

				73.78		100.6291

				73.81		100.6291

				73.83		100.6291

				73.85		100.6291

				73.87		100.6291

				73.89		100.6291

				73.91		100.6291

				73.93		100.6291

				73.95		100.6291

				73.97		100.6291

				73.99		100.6291

				74.02		100.6291

				74.04		100.6291

				74.06		100.6291

				74.08		100.6291

				74.1		100.6291

				74.12		100.6291

				74.14		100.6291

				74.16		100.6291

				74.18		100.6291

				74.2		100.6291

				74.23		100.6291

				74.25		100.6291

				74.27		100.6291

				74.29		100.6291

				74.31		100.6291

				74.33		100.6291

				74.35		100.6291

				74.37		100.6291

				74.39		100.6291

				74.41		100.6291

				74.44		100.6291

				74.46		100.6291

				74.48		100.6291

				74.5		100.6291

				74.52		100.6291

				74.54		100.6291

				74.56		100.6291

				74.58		100.6291

				74.6		100.6291

				74.62		100.6291

				74.65		100.6335

				74.67		100.6335

				74.69		100.6335

				74.71		100.6335

				74.73		100.6335

				74.75		100.6335

				74.77		100.6335

				74.79		100.6335

				74.81		100.6335

				74.83		100.6335

				74.86		100.6335

				74.88		100.6335

				74.9		100.6335

				74.92		100.6335

				74.94		100.6335

				74.96		100.6335

				74.98		100.6335

				75		100.6335

				75.02		100.6335

				75.04		100.6335

				75.07		100.6379

				75.09		100.6379

				75.11		100.6379

				75.13		100.6379

				75.15		100.6379

				75.17		100.6379

				75.19		100.6379

				75.21		100.6379

				75.23		100.6379

				75.25		100.6379

				75.28		100.6379

				75.3		100.6379

				75.32		100.6379

				75.34		100.6379

				75.36		100.6379

				75.38		100.6379

				75.4		100.6379

				75.42		100.6379

				75.44		100.6379

				75.46		100.6379

				75.49		100.6379

				75.51		100.6379

				75.53		100.6379

				75.55		100.6379

				75.57		100.6423

				75.59		100.6423

				75.61		100.6423

				75.63		100.6423

				75.65		100.6423

				75.68		100.6423

				75.7		100.6423

				75.72		100.6423

				75.74		100.6423

				75.76		100.6423

				75.78		100.6423

				75.8		100.6423

				75.82		100.6423

				75.84		100.6423

				75.86		100.6423

				75.89		100.6423

				75.91		100.6423

				75.93		100.6423

				75.95		100.6467

				75.97		100.6467

				75.99		100.6467

				76.01		100.6467

				76.03		100.6467

				76.05		100.6467

				76.07		100.6467

				76.1		100.6467

				76.12		100.6467

				76.14		100.6467

				76.16		100.6467

				76.18		100.6467

				76.2		100.6467

				76.22		100.6467

				76.24		100.6467

				76.26		100.6511

				76.29		100.6511

				76.31		100.6511

				76.33		100.6511

				76.35		100.6511

				76.37		100.6511

				76.39		100.6511

				76.41		100.6511

				76.43		100.6511

				76.45		100.6511

				76.47		100.6511

				76.5		100.6555

				76.52		100.6555

				76.54		100.6555

				76.56		100.6555

				76.58		100.6555

				76.6		100.6555

				76.62		100.6555

				76.64		100.6555

				76.66		100.6555

				76.68		100.6555

				76.71		100.6555

				76.73		100.6555

				76.75		100.6555

				76.77		100.6555

				76.79		100.6555

				76.81		100.6555

				76.83		100.6555

				76.85		100.6555

				76.87		100.6555

				76.9		100.6555

				76.92		100.6555

				76.94		100.6555

				76.96		100.6555

				76.98		100.6555

				77		100.6555

				77.02		100.6555

				77.04		100.6555

				77.06		100.6555

				77.08		100.6555

				77.11		100.6555

				77.13		100.6555

				77.15		100.6555

				77.17		100.6555

				77.19		100.6555

				77.21		100.6555

				77.23		100.6555

				77.25		100.6555

				77.27		100.6555

				77.3		100.6555

				77.32		100.6555

				77.34		100.6555

				77.36		100.6555

				77.38		100.6555

				77.4		100.6555

				77.42		100.6555

				77.44		100.6555

				77.46		100.6555

				77.48		100.6555

				77.51		100.6555

				77.53		100.6555

				77.55		100.6555

				77.57		100.6555

				77.59		100.6555

				77.61		100.6555

				77.63		100.6555

				77.65		100.6555

				77.67		100.6555

				77.69		100.6555

				77.72		100.6555

				77.74		100.6555

				77.76		100.6555

				77.78		100.6555

				77.8		100.6555

				77.82		100.6555

				77.84		100.6555

				77.86		100.6555

				77.88		100.6555

				77.91		100.6555

				77.93		100.6555

				77.95		100.6555

				77.97		100.6555

				77.99		100.6555

				78.01		100.6555

				78.03		100.6555

				78.05		100.6555

				78.07		100.6555

				78.09		100.6555

				78.12		100.6555

				78.14		100.6555

				78.16		100.6555

				78.18		100.6555

				78.2		100.6555

				78.22		100.6555

				78.24		100.6555

				78.26		100.6555

				78.28		100.6555

				78.3		100.6555

				78.33		100.6555

				78.35		100.6555

				78.37		100.6555

				78.39		100.6555

				78.41		100.6555

				78.43		100.6555

				78.45		100.6555

				78.47		100.6555

				78.49		100.6555

				78.52		100.6555

				78.54		100.6555

				78.56		100.6555

				78.58		100.6555

				78.6		100.6555

				78.62		100.6555

				78.64		100.6555

				78.66		100.6555

				78.68		100.6599

				78.7		100.6555

				78.73		100.6555

				78.75		100.6555

				78.77		100.6555

				78.79		100.6599

				78.81		100.6599

				78.83		100.6599

				78.85		100.6599

				78.87		100.6599

				78.89		100.6599

				78.91		100.6599

				78.94		100.6599

				78.96		100.6599

				78.98		100.6599

				79		100.6599

				79.02		100.6599

				79.04		100.6599

				79.06		100.6599

				79.08		100.6599

				79.1		100.6599

				79.12		100.6599

				79.15		100.6599

				79.17		100.6599

				79.19		100.6599

				79.21		100.6599

				79.23		100.6599

				79.25		100.6599

				79.27		100.6599

				79.29		100.6599

				79.31		100.6599

				79.34		100.6599

				79.36		100.6599

				79.38		100.6643

				79.4		100.6643

				79.42		100.6643

				79.44		100.6643

				79.46		100.6643

				79.48		100.6643

				79.5		100.6643

				79.52		100.6643

				79.55		100.6643

				79.57		100.6643

				79.59		100.6643

				79.61		100.6643

				79.63		100.6643

				79.65		100.6643

				79.67		100.6643

				79.69		100.6643

				79.71		100.6643

				79.74		100.6643

				79.76		100.6687

				79.78		100.6643

				79.8		100.6687

				79.82		100.6687

				79.84		100.6687

				79.86		100.6643

				79.88		100.6687

				79.9		100.6687

				79.92		100.6687

				79.95		100.6687

				79.97		100.6687

				79.99		100.6687

				80.01		100.6687

				80.03		100.6643

				80.05		100.6687

				80.07		100.6687

				80.09		100.6687

				80.11		100.6687

				80.14		100.6687

				80.16		100.6687

				80.18		100.6687

				80.2		100.6687

				80.22		100.6687

				80.24		100.6687

				80.26		100.6687

				80.28		100.6687

				80.3		100.6687

				80.32		100.6687

				80.35		100.6687

				80.37		100.6687

				80.39		100.6687

				80.41		100.6687

				80.43		100.6687

				80.45		100.6687

				80.47		100.6687

				80.49		100.6687

				80.51		100.6687

				80.53		100.6687

				80.56		100.6687

				80.58		100.6687

				80.6		100.6731

				80.62		100.6731

				80.64		100.6731

				80.66		100.6731

				80.68		100.6731

				80.7		100.6731

				80.72		100.6731

				80.75		100.6731

				80.77		100.6731

				80.79		100.6731

				80.81		100.6731

				80.83		100.6731

				80.85		100.6731

				80.87		100.6731

				80.89		100.6775

				80.91		100.6775

				80.93		100.6731

				80.96		100.6775

				80.98		100.6775

				81		100.6775

				81.02		100.6775

				81.04		100.6731

				81.06		100.6775

				81.08		100.6731

				81.1		100.6775

				81.12		100.6775

				81.15		100.6775

				81.17		100.6775

				81.19		100.6775

				81.21		100.6775

				81.23		100.6775

				81.25		100.6775

				81.27		100.6775

				81.29		100.6775

				81.31		100.6775

				81.34		100.6775

				81.36		100.6775

				81.38		100.6775

				81.4		100.6775

				81.42		100.6775

				81.44		100.6775

				81.46		100.6775

				81.48		100.6775

				81.5		100.6775

				81.52		100.6775

				81.55		100.6775

				81.57		100.6775

				81.59		100.6775

				81.61		100.6775

				81.63		100.6775

				81.65		100.6775

				81.67		100.6775

				81.69		100.6775

				81.71		100.6775

				81.74		100.6775

				81.76		100.6775

				81.78		100.6775

				81.8		100.6775

				81.82		100.6775

				81.84		100.6775

				81.86		100.6775

				81.88		100.6775

				81.9		100.6775

				81.93		100.6775

				81.95		100.6775

				81.97		100.6775

				81.99		100.6775

				82.01		100.6775

				82.03		100.6775

				82.05		100.6775

				82.07		100.6775

				82.09		100.6775

				82.11		100.6775

				82.14		100.6775

				82.16		100.6775

				82.18		100.6775

				82.2		100.6775

				82.22		100.6775

				82.24		100.6775

				82.26		100.6775

				82.28		100.6819

				82.3		100.6775

				82.33		100.6819

				82.35		100.6819

				82.37		100.6819

				82.39		100.6819

				82.41		100.6819

				82.43		100.6819

				82.45		100.6819

				82.47		100.6819

				82.49		100.6819

				82.51		100.6819

				82.54		100.6819

				82.56		100.6819

				82.58		100.6819

				82.6		100.6819

				82.62		100.6819

				82.64		100.6819

				82.66		100.6819

				82.68		100.6819

				82.7		100.6819

				82.73		100.6819

				82.75		100.6819

				82.77		100.6819

				82.79		100.6819

				82.81		100.6819

				82.83		100.6819

				82.85		100.6819

				82.87		100.6819

				82.89		100.6819

				82.92		100.6819

				82.94		100.6819

				82.96		100.6819

				82.98		100.6819

				83		100.6819

				83.02		100.6819

				83.04		100.6819

				83.06		100.6819

				83.08		100.6819

				83.1		100.6819

				83.13		100.6819

				83.15		100.6819

				83.17		100.6819

				83.19		100.6819

				83.21		100.6819

				83.23		100.6863

				83.25		100.6863

				83.27		100.6863

				83.29		100.6863

				83.32		100.6863

				83.34		100.6863

				83.36		100.6863

				83.38		100.6863

				83.4		100.6863

				83.42		100.6863

				83.44		100.6863

				83.46		100.6863

				83.48		100.6863

				83.51		100.6863

				83.53		100.6863

				83.55		100.6863

				83.57		100.6863

				83.59		100.6863

				83.61		100.6863

				83.63		100.6863

				83.65		100.6863

				83.67		100.6863

				83.69		100.6863

				83.72		100.6907

				83.74		100.6907

				83.76		100.6907

				83.78		100.6907

				83.8		100.6907

				83.82		100.6907

				83.84		100.6907

				83.86		100.6907

				83.88		100.6907

				83.91		100.6907

				83.93		100.6907

				83.95		100.6907

				83.97		100.6907

				83.99		100.6907

				84.01		100.6951

				84.03		100.6951

				84.05		100.6951

				84.07		100.6951

				84.1		100.6951

				84.12		100.6951

				84.14		100.6951

				84.16		100.6951

				84.18		100.6951

				84.2		100.6951

				84.22		100.6951

				84.24		100.6951

				84.26		100.6951

				84.29		100.6951

				84.31		100.6951

				84.33		100.6951

				84.35		100.6951

				84.37		100.6951

				84.39		100.6951

				84.41		100.6951

				84.43		100.6951

				84.45		100.6951

				84.48		100.6951

				84.5		100.6951

				84.52		100.6951

				84.54		100.6951

				84.56		100.6951

				84.58		100.6951

				84.6		100.6951

				84.62		100.6951

				84.64		100.6995

				84.66		100.6995

				84.69		100.6995

				84.71		100.6995

				84.73		100.6995

				84.75		100.6995

				84.77		100.6995

				84.79		100.6995

				84.81		100.6995

				84.83		100.6995

				84.85		100.6995

				84.88		100.6995

				84.9		100.6995

				84.92		100.6995

				84.94		100.6995

				84.96		100.6995

				84.98		100.6995

				85		100.7039

				85.02		100.7039

				85.04		100.6995

				85.07		100.7039

				85.09		100.7039

				85.11		100.7039

				85.13		100.7039

				85.15		100.7039

				85.17		100.7039

				85.19		100.7039

				85.21		100.7039

				85.23		100.7039

				85.26		100.7039

				85.28		100.7039

				85.3		100.7039

				85.32		100.7039

				85.34		100.7039

				85.36		100.7039

				85.38		100.7039

				85.4		100.7039

				85.42		100.7083

				85.44		100.7083

				85.47		100.7083

				85.49		100.7083

				85.51		100.7083

				85.53		100.7083

				85.55		100.7083

				85.57		100.7083

				85.59		100.7083

				85.61		100.7083

				85.63		100.7083

				85.66		100.7083

				85.68		100.7083

				85.7		100.7083

				85.72		100.7083

				85.74		100.7083

				85.76		100.7083

				85.78		100.7083

				85.8		100.7083

				85.82		100.7083

				85.84		100.7083

				85.87		100.7083

				85.89		100.7083

				85.91		100.7127

				85.93		100.7083

				85.95		100.7083

				85.97		100.7083

				85.99		100.7083

				86.01		100.7127

				86.03		100.7083

				86.06		100.7127

				86.08		100.7127

				86.1		100.7127

				86.12		100.7127

				86.14		100.7127

				86.16		100.7127

				86.18		100.7127

				86.2		100.7127

				86.22		100.7127

				86.24		100.7127

				86.27		100.7127

				86.29		100.7127

				86.31		100.7127

				86.33		100.7127

				86.35		100.7127

				86.37		100.7127

				86.39		100.7127

				86.41		100.7127

				86.43		100.7171

				86.46		100.7171

				86.48		100.7171

				86.5		100.7171

				86.52		100.7171

				86.54		100.7171

				86.56		100.7171

				86.58		100.7171

				86.6		100.7171

				86.62		100.7171

				86.65		100.7171

				86.67		100.7171

				86.69		100.7171

				86.71		100.7171

				86.73		100.7171

				86.75		100.7171

				86.77		100.7171

				86.79		100.7171

				86.81		100.7171

				86.83		100.7171

				86.86		100.7171

				86.88		100.7171

				86.9		100.7171

				86.92		100.7171

				86.94		100.7171

				86.96		100.7171

				86.98		100.7171

				87		100.7171

				87.02		100.7171

				87.05		100.7171

				87.07		100.7171

				87.09		100.7171

				87.11		100.7171

				87.13		100.7171

				87.15		100.7171

				87.17		100.7171

				87.19		100.7171

				87.21		100.7171

				87.23		100.7171

				87.26		100.7171

				87.28		100.7171

				87.3		100.7171

				87.32		100.7171

				87.34		100.7171

				87.36		100.7171

				87.38		100.7171

				87.4		100.7171

				87.42		100.7171

				87.45		100.7171

				87.47		100.7171

				87.49		100.7171

				87.51		100.7171

				87.53		100.7171

				87.55		100.7171

				87.57		100.7171

				87.59		100.7171

				87.61		100.7171

				87.63		100.7171

				87.66		100.7171

				87.68		100.7171

				87.7		100.7171

				87.72		100.7171

				87.74		100.7171

				87.76		100.7171

				87.78		100.7171

				87.8		100.7171

				87.82		100.7171

				87.85		100.7171

				87.87		100.7171

				87.89		100.7171

				87.91		100.7171

				87.93		100.7171

				87.95		100.7171

				87.97		100.7171

				87.99		100.7171

				88.01		100.7171

				88.03		100.7171

				88.06		100.7171

				88.08		100.7171

				88.1		100.7127

				88.12		100.7171

				88.14		100.7171

				88.16		100.7127

				88.18		100.7171

				88.2		100.7171

				88.22		100.7127

				88.25		100.7127

				88.27		100.7127

				88.29		100.7127

				88.31		100.7127

				88.33		100.7127

				88.35		100.7171

				88.37		100.7171

				88.39		100.7171

				88.41		100.7127

				88.43		100.7127

				88.46		100.7171

				88.48		100.7127

				88.5		100.7171

				88.52		100.7127

				88.54		100.7127

				88.56		100.7127

				88.58		100.7171

				88.6		100.7171

				88.62		100.7127

				88.65		100.7171

				88.67		100.7127

				88.69		100.7127

				88.71		100.7171

				88.73		100.7127

				88.75		100.7171

				88.77		100.7171

				88.79		100.7171

				88.81		100.7171

				88.83		100.7171

				88.86		100.7171

				88.88		100.7171

				88.9		100.7171

				88.92		100.7171

				88.94		100.7171

				88.96		100.7171

				88.98		100.7171

				89		100.7171

				89.02		100.7171

				89.05		100.7171

				89.07		100.7171

				89.09		100.7171

				89.11		100.7171

				89.13		100.7171

				89.15		100.7171

				89.17		100.7171

				89.19		100.7171

				89.21		100.7171

				89.24		100.7171

				89.26		100.7171

				89.28		100.7171

				89.3		100.7171

				89.32		100.7171

				89.34		100.7171

				89.36		100.7171

				89.38		100.7171

				89.4		100.7171

				89.42		100.7215

				89.45		100.7215

				89.47		100.7215

				89.49		100.7215

				89.51		100.7215

				89.53		100.7215

				89.55		100.7215

				89.57		100.7215

				89.59		100.7215

				89.61		100.7215

				89.64		100.7215

				89.66		100.7215

				89.68		100.7215

				89.7		100.7215

				89.72		100.7215

				89.74		100.7215

				89.76		100.7215

				89.78		100.7215

				89.8		100.7215

				89.82		100.7215

				89.85		100.7215

				89.87		100.7215

				89.89		100.7215

				89.91		100.7215

				89.93		100.7215

				89.95		100.7215

				89.97		100.7215

				89.99		100.7215

				90.01		100.7215

				90.04		100.7215

				90.06		100.7259

				90.08		100.7259

				90.1		100.7259

				90.12		100.7259

				90.14		100.7259

				90.16		100.7259

				90.18		100.7259

				90.2		100.7259

				90.23		100.7259

				90.25		100.7259

				90.27		100.7259

				90.29		100.7259

				90.31		100.7259

				90.33		100.7259

				90.35		100.7259

				90.37		100.7259

				90.39		100.7259

				90.41		100.7259

				90.44		100.7259

				90.46		100.7303

				90.48		100.7259

				90.5		100.7303

				90.52		100.7303

				90.54		100.7303

				90.56		100.7303

				90.58		100.7303

				90.6		100.7303

				90.63		100.7303

				90.65		100.7303

				90.67		100.7303

				90.69		100.7303

				90.71		100.7303

				90.73		100.7303

				90.75		100.7303

				90.77		100.7303

				90.79		100.7303

				90.82		100.7303

				90.84		100.7303

				90.86		100.7303

				90.88		100.7303

				90.9		100.7303

				90.92		100.7347

				90.94		100.7303

				90.96		100.7347

				90.98		100.7347

				91		100.7347

				91.03		100.7347

				91.05		100.7347

				91.07		100.7347

				91.09		100.7347

				91.11		100.7347

				91.13		100.7347

				91.15		100.7347

				91.17		100.7347

				91.19		100.7347

				91.22		100.7347

				91.24		100.7347

				91.26		100.7347

				91.28		100.7347

				91.3		100.7347

				91.32		100.7347

				91.34		100.7347

				91.36		100.7347

				91.38		100.7347

				91.4		100.7347

				91.43		100.7347

				91.45		100.7347

				91.47		100.7347

				91.49		100.7347

				91.51		100.7347

				91.53		100.7347

				91.55		100.7347

				91.57		100.7347

				91.59		100.7347

				91.62		100.7347

				91.64		100.7347

				91.66		100.7347

				91.68		100.7347

				91.7		100.7347

				91.72		100.7347

				91.74		100.7347

				91.76		100.7347

				91.78		100.7347

				91.8		100.7391

				91.83		100.7391

				91.85		100.7391

				91.87		100.7391

				91.89		100.7391

				91.91		100.7347

				91.93		100.7391

				91.95		100.7391

				91.97		100.7391

				91.99		100.7391

				92.02		100.7391

				92.04		100.7391

				92.06		100.7391

				92.08		100.7391

				92.1		100.7391

				92.12		100.7391

				92.14		100.7391

				92.16		100.7391

				92.18		100.7347

				92.2		100.7347

				92.23		100.7391

				92.25		100.7347

				92.27		100.7347

				92.29		100.7391

				92.31		100.7391

				92.33		100.7391

				92.35		100.7347

				92.37		100.7347

				92.39		100.7391

				92.42		100.7391

				92.44		100.7391

				92.46		100.7391

				92.48		100.7391

				92.5		100.7391

				92.52		100.7391

				92.54		100.7391

				92.56		100.7391

				92.58		100.7391

				92.6		100.7391

				92.63		100.7391

				92.65		100.7391

				92.67		100.7391

				92.69		100.7391

				92.71		100.7391

				92.73		100.7391

				92.75		100.7391

				92.77		100.7391

				92.79		100.7391

				92.82		100.7391

				92.84		100.7347

				92.86		100.7391

				92.88		100.7391

				92.9		100.7391

				92.92		100.7391

				92.94		100.7391

				92.96		100.7391

				92.98		100.7391

				93		100.7391

				93.03		100.7391

				93.05		100.7391

				93.07		100.7391

				93.09		100.7391

				93.11		100.7391

				93.13		100.7391

				93.15		100.7391

				93.17		100.7391

				93.19		100.7391

				93.22		100.7391

				93.24		100.7391

				93.26		100.7391

				93.28		100.7391

				93.3		100.7391

				93.32		100.7391

				93.34		100.7391

				93.36		100.7391

				93.38		100.7391

				93.41		100.7391

				93.43		100.7391

				93.45		100.7391

				93.47		100.7391

				93.49		100.7391

				93.51		100.7391

				93.53		100.7391

				93.55		100.7391

				93.57		100.7391

				93.59		100.7391

				93.62		100.7391

				93.64		100.7391

				93.66		100.7391

				93.68		100.7391

				93.7		100.7391

				93.72		100.7391

				93.74		100.7391

				93.76		100.7391

				93.78		100.7391

				93.81		100.7391

				93.83		100.7391

				93.85		100.7391

				93.87		100.7391

				93.89		100.7391

				93.91		100.7391

				93.93		100.7391

				93.95		100.7391

				93.97		100.7391

				93.99		100.7435

				94.02		100.7391

				94.04		100.7391

				94.06		100.7435

				94.08		100.7435

				94.1		100.7435

				94.12		100.7435

				94.14		100.7435

				94.16		100.7435

				94.18		100.7435

				94.21		100.7435

				94.23		100.7435

				94.25		100.7435

				94.27		100.7435

				94.29		100.7435

				94.31		100.7435

				94.33		100.7435

				94.35		100.7435

				94.37		100.7435

				94.39		100.7435

				94.42		100.7435

				94.44		100.7435

				94.46		100.7435

				94.48		100.7435

				94.5		100.7435

				94.52		100.7435

				94.54		100.7435

				94.56		100.7435

				94.58		100.7435

				94.61		100.7479

				94.63		100.7435

				94.65		100.7479

				94.67		100.7479

				94.69		100.7479

				94.71		100.7479

				94.73		100.7479

				94.75		100.7479

				94.77		100.7479

				94.79		100.7479

				94.82		100.7479

				94.84		100.7479

				94.86		100.7479

				94.88		100.7479

				94.9		100.7479

				94.92		100.7479

				94.94		100.7479

				94.96		100.7479

				94.98		100.7479

				95.01		100.7479

				95.03		100.7479

				95.05		100.7479

				95.07		100.7479

				95.09		100.7523

				95.11		100.7523

				95.13		100.7523

				95.15		100.7523

				95.17		100.7523

				95.19		100.7523

				95.22		100.7523

				95.24		100.7523

				95.26		100.7523

				95.28		100.7523

				95.3		100.7523

				95.32		100.7523

				95.34		100.7523

				95.36		100.7523

				95.38		100.7523

				95.4		100.7523

				95.43		100.7523

				95.45		100.7523

				95.47		100.7523

				95.49		100.7567

				95.51		100.7567

				95.53		100.7567

				95.55		100.7567

				95.57		100.7567

				95.59		100.7567

				95.62		100.7567

				95.64		100.7567

				95.66		100.7567

				95.68		100.7567

				95.7		100.7567

				95.72		100.7567

				95.74		100.7567

				95.76		100.7567

				95.78		100.7567

				95.8		100.7567

				95.83		100.7567

				95.85		100.7567

				95.87		100.7567

				95.89		100.7567

				95.91		100.7567

				95.93		100.7567

				95.95		100.7567

				95.97		100.7567

				95.99		100.7567

				96.02		100.7567

				96.04		100.7611

				96.06		100.7611

				96.08		100.7611

				96.1		100.7611

				96.12		100.7611

				96.14		100.7611

				96.16		100.7611

				96.18		100.7611

				96.2		100.7611

				96.23		100.7611

				96.25		100.7611

				96.27		100.7611

				96.29		100.7655

				96.31		100.7655

				96.33		100.7655

				96.35		100.7655

				96.37		100.7655

				96.39		100.7655

				96.42		100.7655

				96.44		100.7655

				96.46		100.7655

				96.48		100.7655

				96.5		100.7655

				96.52		100.7655

				96.54		100.7655

				96.56		100.7655

				96.58		100.7655

				96.61		100.7655

				96.63		100.7655

				96.65		100.7655

				96.67		100.7655

				96.69		100.7655

				96.71		100.7655

				96.73		100.7655

				96.75		100.7655

				96.77		100.7655

				96.79		100.7655

				96.82		100.7655

				96.84		100.7655

				96.86		100.7655

				96.88		100.7699

				96.9		100.7699

				96.92		100.7699

				96.94		100.7699

				96.96		100.7699

				96.98		100.7699

				97.01		100.7699

				97.03		100.7699

				97.05		100.7699

				97.07		100.7699

				97.09		100.7699

				97.11		100.7699

				97.13		100.7699

				97.15		100.7699

				97.17		100.7699

				97.19		100.7699

				97.22		100.7699

				97.24		100.7699

				97.26		100.7699

				97.28		100.7699

				97.3		100.7699

				97.32		100.7699

				97.34		100.7743

				97.36		100.7743

				97.38		100.7743

				97.41		100.7743

				97.43		100.7743

				97.45		100.7743

				97.47		100.7743

				97.49		100.7743

				97.51		100.7743

				97.53		100.7699

				97.55		100.7743

				97.57		100.7699

				97.59		100.7699

				97.62		100.7699

				97.64		100.7699

				97.66		100.7699

				97.68		100.7743

				97.7		100.7743

				97.72		100.7743

				97.74		100.7743

				97.76		100.7743

				97.78		100.7743

				97.8		100.7743

				97.83		100.7743

				97.85		100.7743

				97.87		100.7743

				97.89		100.7743

				97.91		100.7743

				97.93		100.7743

				97.95		100.7743

				97.97		100.7743

				97.99		100.7743

				98.02		100.7743

				98.04		100.7743

				98.06		100.7743

				98.08		100.7787

				98.1		100.7787

				98.12		100.7787

				98.14		100.7787

				98.16		100.7787

				98.18		100.7787

				98.2		100.7787

				98.23		100.7787

				98.25		100.7787

				98.27		100.7787

				98.29		100.7787

				98.31		100.7787

				98.33		100.7787

				98.35		100.7787

				98.37		100.7743

				98.39		100.7787

				98.42		100.7787

				98.44		100.7787

				98.46		100.7787

				98.48		100.7787

				98.5		100.7787

				98.52		100.7787

				98.54		100.7787

				98.56		100.7787

				98.58		100.7787

				98.6		100.7787

				98.63		100.7787

				98.65		100.7787

				98.67		100.7787

				98.69		100.7787

				98.71		100.7787

				98.73		100.7787

				98.75		100.7787

				98.77		100.7787

				98.79		100.7787

				98.82		100.7787

				98.84		100.7787

				98.86		100.7787

				98.88		100.7787

				98.9		100.7787

				98.92		100.7787

				98.94		100.7787

				98.96		100.7787

				98.98		100.7787

				99		100.7787

				99.03		100.7787

				99.05		100.7787

				99.07		100.7787

				99.09		100.7787

				99.11		100.7787

				99.13		100.7787

				99.15		100.7787

				99.17		100.7787

				99.19		100.7787

				99.22		100.7787

				99.24		100.7787

				99.26		100.7787

				99.28		100.7787

				99.3		100.7787

				99.32		100.7787

				99.34		100.7787

				99.36		100.7787

				99.38		100.7787

				99.4		100.7787

				99.43		100.7787

				99.45		100.7787

				99.47		100.7787

				99.49		100.7787

				99.51		100.7787

				99.53		100.7787

				99.55		100.7787

				99.57		100.7787

				99.59		100.7787

				99.61		100.7787

				99.64		100.7787

				99.66		100.7787

				99.68		100.7787

				99.7		100.7787

				99.72		100.7787

				99.74		100.7787

				99.76		100.7787

				99.78		100.7787

				99.8		100.7743

				99.83		100.7743

				99.85		100.7743

				99.87		100.7743

				99.89		100.7743

				99.91		100.7743

				99.93		100.7743

				99.95		100.7743

				99.97		100.7743

				99.99		100.7743

				100.01		100.7743

				100.04		100.7743

				100.06		100.7743

				100.08		100.7743

				100.1		100.7743

				100.12		100.7743

				100.14		100.7743

				100.16		100.7743

				100.18		100.7743

				100.2		100.7743

				100.22		100.7743

				100.25		100.7743

				100.27		100.7743

				100.29		100.7743

				100.31		100.7743

				100.33		100.7743

				100.35		100.7743

				100.37		100.7743

				100.39		100.7743

				100.41		100.7743

				100.44		100.7743

				100.46		100.7743

				100.48		100.7743

				100.5		100.7743

				100.52		100.7743

				100.54		100.7743

				100.56		100.7787

				100.58		100.7743

				100.6		100.7787

				100.62		100.7787

				100.65		100.7787

				100.67		100.7787

				100.69		100.7787

				100.71		100.7787

				100.73		100.7787

				100.75		100.7787

				100.77		100.7787

				100.79		100.7787

				100.81		100.7787

				100.84		100.7787

				100.86		100.7787

				100.88		100.7787

				100.9		100.7787

				100.92		100.7787

				100.94		100.7787

				100.96		100.7787

				100.98		100.7787

				101		100.7787

				101.02		100.7787

				101.05		100.7787

				101.07		100.7787

				101.09		100.7787

				101.11		100.7787

				101.13		100.7787

				101.15		100.7787

				101.17		100.7787

				101.19		100.7787

				101.21		100.7831

				101.23		100.7831

				101.26		100.7831

				101.28		100.7831

				101.3		100.7831

				101.32		100.7831

				101.34		100.7831

				101.36		100.7831

				101.38		100.7831

				101.4		100.7831

				101.42		100.7831

				101.44		100.7831

				101.47		100.7831

				101.49		100.7831

				101.51		100.7831

				101.53		100.7831

				101.55		100.7831

				101.57		100.7831

				101.59		100.7831

				101.61		100.7831

				101.63		100.7831

				101.66		100.7831

				101.68		100.7831

				101.7		100.7831

				101.72		100.7831

				101.74		100.7875

				101.76		100.7875

				101.78		100.7875

				101.8		100.7875

				101.82		100.7875

				101.84		100.7875

				101.87		100.7875

				101.89		100.7875

				101.91		100.7875

				101.93		100.7875

				101.95		100.7875

				101.97		100.7875

				101.99		100.7875

				102.01		100.7875

				102.03		100.7875

				102.05		100.7875

				102.08		100.7875

				102.1		100.7875

				102.12		100.7875

				102.14		100.7919

				102.16		100.7919

				102.18		100.7875

				102.2		100.7919

				102.22		100.7919

				102.24		100.7919

				102.26		100.7875

				102.29		100.7919

				102.31		100.7919

				102.33		100.7919

				102.35		100.7919

				102.37		100.7919

				102.39		100.7919

				102.41		100.7919

				102.43		100.7919

				102.45		100.7919

				102.48		100.7919

				102.5		100.7919

				102.52		100.7919

				102.54		100.7919

				102.56		100.7919

				102.58		100.7919

				102.6		100.7875

				102.62		100.7875

				102.64		100.7875

				102.66		100.7875

				102.69		100.7875

				102.71		100.7875

				102.73		100.7875

				102.75		100.7875

				102.77		100.7875

				102.79		100.7875

				102.81		100.7875

				102.83		100.7875

				102.85		100.7875

				102.87		100.7875

				102.9		100.7875

				102.92		100.7875

				102.94		100.7875

				102.96		100.7875

				102.98		100.7875

				103		100.7875

				103.02		100.7875

				103.04		100.7875

				103.06		100.7875

				103.09		100.7875

				103.11		100.7875

				103.13		100.7875

				103.15		100.7875

				103.17		100.7875

				103.19		100.7875

				103.21		100.7875

				103.23		100.7875

				103.25		100.7875

				103.27		100.7875

				103.3		100.7875

				103.32		100.7875

				103.34		100.7875

				103.36		100.7875

				103.38		100.7875

				103.4		100.7875

				103.42		100.7875

				103.44		100.7875

				103.46		100.7875

				103.49		100.7875

				103.51		100.7875

				103.53		100.7875

				103.55		100.7875

				103.57		100.7875

				103.59		100.7875

				103.61		100.7875

				103.63		100.7875

				103.65		100.7875

				103.67		100.7875

				103.7		100.7875

				103.72		100.7875

				103.74		100.7875

				103.76		100.7875

				103.78		100.7875

				103.8		100.7875

				103.82		100.7875

				103.84		100.7875

				103.86		100.7875

				103.88		100.7875

				103.91		100.7875

				103.93		100.7875

				103.95		100.7831

				103.97		100.7875

				103.99		100.7831

				104.01		100.7875

				104.03		100.7875

				104.05		100.7831

				104.07		100.7831

				104.1		100.7831

				104.12		100.7831

				104.14		100.7831

				104.16		100.7831

				104.18		100.7831

				104.2		100.7831

				104.22		100.7831

				104.24		100.7831

				104.26		100.7875

				104.28		100.7831

				104.31		100.7875

				104.33		100.7875

				104.35		100.7875

				104.37		100.7831

				104.39		100.7875

				104.41		100.7875

				104.43		100.7875

				104.45		100.7875

				104.47		100.7875

				104.49		100.7875

				104.52		100.7875

				104.54		100.7875

				104.56		100.7875

				104.58		100.7875

				104.6		100.7875

				104.62		100.7875

				104.64		100.7875

				104.66		100.7875

				104.68		100.7875

				104.71		100.7875

				104.73		100.7875

				104.75		100.7875

				104.77		100.7875

				104.79		100.7875

				104.81		100.7875

				104.83		100.7875

				104.85		100.7875

				104.87		100.7875

				104.89		100.7875

				104.92		100.7875

				104.94		100.7875

				104.96		100.7875

				104.98		100.7875

				105		100.7875

				105.02		100.7875

				105.04		100.7875

				105.06		100.7875

				105.08		100.7875

				105.1		100.7875

				105.13		100.7875

				105.15		100.7875

				105.17		100.7875

				105.19		100.7875

				105.21		100.7875

				105.23		100.7875

				105.25		100.7875

				105.27		100.7875

				105.29		100.7875

				105.32		100.7875

				105.34		100.7875

				105.36		100.7875

				105.38		100.7831

				105.4		100.7831

				105.42		100.7831

				105.44		100.7831

				105.46		100.7831

				105.48		100.7831

				105.5		100.7831

				105.53		100.7831

				105.55		100.7831

				105.57		100.7831

				105.59		100.7831

				105.61		100.7831

				105.63		100.7831

				105.65		100.7831

				105.67		100.7831

				105.69		100.7831

				105.71		100.7831

				105.74		100.7831

				105.76		100.7875

				105.78		100.7875

				105.8		100.7831

				105.82		100.7831

				105.84		100.7831

				105.86		100.7831

				105.88		100.7875

				105.9		100.7875

				105.93		100.7875

				105.95		100.7875

				105.97		100.7831

				105.99		100.7875

				106.01		100.7875

				106.03		100.7875

				106.05		100.7875

				106.07		100.7875

				106.09		100.7875

				106.11		100.7875

				106.14		100.7875

				106.16		100.7875

				106.18		100.7875

				106.2		100.7875

				106.22		100.7875

				106.24		100.7831

				106.26		100.7831

				106.28		100.7831

				106.3		100.7831

				106.32		100.7831

				106.35		100.7831

				106.37		100.7831

				106.39		100.7875

				106.41		100.7831

				106.43		100.7831

				106.45		100.7875

				106.47		100.7875

				106.49		100.7875

				106.51		100.7875

				106.54		100.7875

				106.56		100.7875

				106.58		100.7831

				106.6		100.7831

				106.62		100.7831

				106.64		100.7831

				106.66		100.7831

				106.68		100.7831

				106.7		100.7831

				106.72		100.7831

				106.75		100.7831

				106.77		100.7831

				106.79		100.7831

				106.81		100.7831

				106.83		100.7831

				106.85		100.7831

				106.87		100.7831

				106.89		100.7831

				106.91		100.7831

				106.93		100.7831

				106.96		100.7831

				106.98		100.7831

				107		100.7831

				107.02		100.7831

				107.04		100.7875

				107.06		100.7875

				107.08		100.7875

				107.1		100.7875

				107.12		100.7875

				107.14		100.7875

				107.17		100.7875

				107.19		100.7875

				107.21		100.7875

				107.23		100.7875

				107.25		100.7875

				107.27		100.7875

				107.29		100.7875

				107.31		100.7875

				107.33		100.7875

				107.36		100.7875

				107.38		100.7875

				107.4		100.7875

				107.42		100.7875

				107.44		100.7875

				107.46		100.7875

				107.48		100.7875

				107.5		100.7875

				107.52		100.7875

				107.54		100.7875

				107.57		100.7875

				107.59		100.7875

				107.61		100.7875

				107.63		100.7875

				107.65		100.7875

				107.67		100.7875

				107.69		100.7875

				107.71		100.7875

				107.73		100.7919

				107.75		100.7875

				107.78		100.7919

				107.8		100.7875

				107.82		100.7919

				107.84		100.7875

				107.86		100.7875

				107.88		100.7919

				107.9		100.7875

				107.92		100.7919

				107.94		100.7919

				107.96		100.7919

				107.99		100.7919

				108.01		100.7919

				108.03		100.7919

				108.05		100.7919

				108.07		100.7919

				108.09		100.7919

				108.11		100.7919

				108.13		100.7919

				108.15		100.7919

				108.17		100.7919

				108.2		100.7919

				108.22		100.7919

				108.24		100.7919

				108.26		100.7919

				108.28		100.7919

				108.3		100.7919

				108.32		100.7919

				108.34		100.7919

				108.36		100.7919

				108.39		100.7919

				108.41		100.7919

				108.43		100.7919

				108.45		100.7963

				108.47		100.7963

				108.49		100.7963

				108.51		100.7963

				108.53		100.7963

				108.55		100.7963

				108.57		100.7963

				108.6		100.7919

				108.62		100.7963

				108.64		100.7963

				108.66		100.7963

				108.68		100.7963

				108.7		100.7963

				108.72		100.7963

				108.74		100.7963

				108.76		100.7963

				108.78		100.7963

				108.81		100.7963

				108.83		100.7963

				108.85		100.7963

				108.87		100.7963

				108.89		100.7963

				108.91		100.7963

				108.93		100.7963

				108.95		100.7963

				108.97		100.7963

				108.99		100.7963

				109.02		100.7963

				109.04		100.7963

				109.06		100.7963

				109.08		100.7963

				109.1		100.7963

				109.12		100.7963

				109.14		100.7963

				109.16		100.8007

				109.18		100.8007

				109.2		100.8007

				109.23		100.8007

				109.25		100.8007

				109.27		100.8007

				109.29		100.8007

				109.31		100.8007

				109.33		100.8007

				109.35		100.8007

				109.37		100.8007

				109.39		100.8007

				109.41		100.8007

				109.44		100.8007

				109.46		100.8007

				109.48		100.8007

				109.5		100.8007

				109.52		100.8007

				109.54		100.8007

				109.56		100.8007

				109.58		100.8007

				109.6		100.8007

				109.62		100.8007

				109.65		100.8007

				109.67		100.8007

				109.69		100.8007

				109.71		100.8007

				109.73		100.8007

				109.75		100.8007

				109.77		100.8007

				109.79		100.8007

				109.81		100.8007

				109.84		100.8007

				109.86		100.8007

				109.88		100.8007

				109.9		100.8007

				109.92		100.8007

				109.94		100.8007

				109.96		100.8007

				109.98		100.8007

				110		100.8007

				110.02		100.8007

				110.05		100.8007

				110.07		100.8007

				110.09		100.8007

				110.11		100.8007

				110.13		100.8007

				110.15		100.8007

				110.17		100.8007

				110.19		100.8007

				110.21		100.8007

				110.23		100.8007

				110.26		100.8007

				110.28		100.8007

				110.3		100.8007

				110.32		100.8007

				110.34		100.8007

				110.36		100.8007

				110.38		100.8007

				110.4		100.8007

				110.42		100.8007

				110.44		100.8007

				110.47		100.8007

				110.49		100.8007

				110.51		100.8007

				110.53		100.8007

				110.55		100.8007

				110.57		100.8007

				110.59		100.8007

				110.61		100.8007

				110.63		100.8007

				110.65		100.8007

				110.68		100.8007

				110.7		100.8007

				110.72		100.8007

				110.74		100.8007

				110.76		100.8007

				110.78		100.8007

				110.8		100.8007

				110.82		100.8007

				110.84		100.8007

				110.87		100.8007

				110.89		100.8007

				110.91		100.8007

				110.93		100.8007

				110.95		100.8007

				110.97		100.8007

				110.99		100.8007

				111.01		100.8007

				111.03		100.8007

				111.05		100.8007

				111.08		100.8007

				111.1		100.8007

				111.12		100.8007

				111.14		100.8007

				111.16		100.8007

				111.18		100.8007

				111.2		100.8051

				111.22		100.8051

				111.24		100.8051

				111.26		100.8007

				111.29		100.8007

				111.31		100.8007

				111.33		100.8007

				111.35		100.8007

				111.37		100.8007

				111.39		100.8007

				111.41		100.8007

				111.43		100.8007

				111.45		100.8051

				111.47		100.8051

				111.5		100.8007

				111.52		100.8051

				111.54		100.8051

				111.56		100.8051

				111.58		100.8051

				111.6		100.8051

				111.62		100.8051

				111.64		100.8051

				111.66		100.8051

				111.68		100.8051

				111.71		100.8051

				111.73		100.8051

				111.75		100.8051

				111.77		100.8051

				111.79		100.8051

				111.81		100.8051

				111.83		100.8051

				111.85		100.8051

				111.87		100.8051

				111.89		100.8051

				111.92		100.8051

				111.94		100.8051

				111.96		100.8051

				111.98		100.8051

				112		100.8051

				112.02		100.8051

				112.04		100.8051

				112.06		100.8051

				112.08		100.8051

				112.1		100.8051

				112.13		100.8051

				112.15		100.8051

				112.17		100.8095

				112.19		100.8095

				112.21		100.8095

				112.23		100.8095

				112.25		100.8095

				112.27		100.8095

				112.29		100.8095

				112.31		100.8095

				112.34		100.8095

				112.36		100.8095

				112.38		100.8095

				112.4		100.8095

				112.42		100.8095

				112.44		100.8095

				112.46		100.8095

				112.48		100.8095

				112.5		100.8095

				112.53		100.8095

				112.55		100.8095

				112.57		100.8095

				112.59		100.8095

				112.61		100.8095

				112.63		100.8095

				112.65		100.8095

				112.67		100.8095

				112.69		100.8095

				112.71		100.8095

				112.74		100.8095

				112.76		100.8095

				112.78		100.8095

				112.8		100.8095

				112.82		100.8095

				112.84		100.8095

				112.86		100.8095

				112.88		100.8095

				112.9		100.8095

				112.92		100.8095

				112.94		100.8095

				112.97		100.8095

				112.99		100.8095

				113.01		100.8095

				113.03		100.8095

				113.05		100.8095

				113.07		100.8095

				113.09		100.8095

				113.11		100.8095

				113.13		100.8095

				113.15		100.8095

				113.18		100.8095

				113.2		100.8095

				113.22		100.8095

				113.24		100.8095

				113.26		100.8095

				113.28		100.8095

				113.3		100.8095

				113.32		100.8095

				113.34		100.8095

				113.36		100.8095

				113.39		100.8095

				113.41		100.8095

				113.43		100.8095

				113.45		100.8095

				113.47		100.8095

				113.49		100.8095

				113.51		100.8095

				113.53		100.8095

				113.55		100.8095

				113.57		100.8095

				113.6		100.8095

				113.62		100.8095

				113.64		100.8095

				113.66		100.8095

				113.68		100.8095

				113.7		100.8095

				113.72		100.8095

				113.74		100.8095

				113.76		100.8095

				113.78		100.8095

				113.81		100.8095

				113.83		100.8095

				113.85		100.8095

				113.87		100.8095

				113.89		100.8095

				113.91		100.8095

				113.93		100.8095

				113.95		100.8095

				113.97		100.8095

				113.99		100.8095

				114.02		100.8095

				114.04		100.8095

				114.06		100.8095

				114.08		100.8095

				114.1		100.8095

				114.12		100.8095

				114.14		100.8095

				114.16		100.8095

				114.18		100.8095

				114.21		100.8095

				114.23		100.8051

				114.25		100.8051

				114.27		100.8051

				114.29		100.8051

				114.31		100.8051

				114.33		100.8051

				114.35		100.8051

				114.37		100.8051

				114.39		100.8051

				114.42		100.8051

				114.44		100.8051

				114.46		100.8051

				114.48		100.8051

				114.5		100.8051

				114.52		100.8051

				114.54		100.8051

				114.56		100.8051

				114.58		100.8051

				114.6		100.8051

				114.63		100.8051

				114.65		100.8051

				114.67		100.8051

				114.69		100.8095

				114.71		100.8095

				114.73		100.8095

				114.75		100.8095

				114.77		100.8095

				114.79		100.8051

				114.81		100.8095

				114.84		100.8051

				114.86		100.8051

				114.88		100.8051

				114.9		100.8051

				114.92		100.8095

				114.94		100.8095

				114.96		100.8051

				114.98		100.8095

				115		100.8095

				115.02		100.8095

				115.05		100.8095

				115.07		100.8095

				115.09		100.8095

				115.11		100.8095

				115.13		100.8095

				115.15		100.8095

				115.17		100.8095

				115.19		100.8095

				115.21		100.8095

				115.23		100.8095

				115.26		100.8095

				115.28		100.8095

				115.3		100.8095

				115.32		100.8095

				115.34		100.8095

				115.36		100.8095

				115.38		100.8095

				115.4		100.8095

				115.42		100.8095

				115.44		100.8095

				115.47		100.8095

				115.49		100.8095

				115.51		100.8095

				115.53		100.8095

				115.55		100.8095

				115.57		100.8095

				115.59		100.8095

				115.61		100.8095

				115.63		100.8095

				115.65		100.8139

				115.68		100.8139

				115.7		100.8139

				115.72		100.8139

				115.74		100.8139

				115.76		100.8139

				115.78		100.8139

				115.8		100.8139

				115.82		100.8095

				115.84		100.8095

				115.86		100.8095

				115.89		100.8095

				115.91		100.8095

				115.93		100.8095

				115.95		100.8095

				115.97		100.8095

				115.99		100.8095

				116.01		100.8095

				116.03		100.8095

				116.05		100.8095

				116.07		100.8095

				116.1		100.8095

				116.12		100.8095

				116.14		100.8095

				116.16		100.8095

				116.18		100.8095

				116.2		100.8095

				116.22		100.8095

				116.24		100.8095

				116.26		100.8095

				116.29		100.8095

				116.31		100.8095

				116.33		100.8095

				116.35		100.8095

				116.37		100.8095

				116.39		100.8095

				116.41		100.8095

				116.43		100.8095

				116.45		100.8095

				116.47		100.8139

				116.5		100.8139

				116.52		100.8139

				116.54		100.8139

				116.56		100.8139

				116.58		100.8139

				116.6		100.8139

				116.62		100.8139

				116.64		100.8139

				116.66		100.8139

				116.68		100.8095

				116.71		100.8095

				116.73		100.8139

				116.75		100.8095

				116.77		100.8095

				116.79		100.8095

				116.81		100.8095

				116.83		100.8095

				116.85		100.8095

				116.87		100.8095

				116.89		100.8095

				116.92		100.8095

				116.94		100.8095

				116.96		100.8095

				116.98		100.8095

				117		100.8095

				117.02		100.8095

				117.04		100.8095

				117.06		100.8095

				117.08		100.8095

				117.1		100.8095

				117.13		100.8095

				117.15		100.8095

				117.17		100.8095

				117.19		100.8095

				117.21		100.8095

				117.23		100.8095

				117.25		100.8095

				117.27		100.8095

				117.29		100.8095

				117.31		100.8095

				117.34		100.8095

				117.36		100.8095

				117.38		100.8095

				117.4		100.8095

				117.42		100.8095

				117.44		100.8095

				117.46		100.8095

				117.48		100.8095

				117.5		100.8095

				117.52		100.8095

				117.55		100.8095

				117.57		100.8095

				117.59		100.8095

				117.61		100.8095

				117.63		100.8095

				117.65		100.8095

				117.67		100.8095

				117.69		100.8095

				117.71		100.8095

				117.73		100.8095

				117.76		100.8095

				117.78		100.8095

				117.8		100.8095

				117.82		100.8095

				117.84		100.8095

				117.86		100.8095

				117.88		100.8095

				117.9		100.8095

				117.92		100.8095

				117.94		100.8095

				117.97		100.8095

				117.99		100.8095

				118.01		100.8095

				118.03		100.8095

				118.05		100.8095

				118.07		100.8095

				118.09		100.8095

				118.11		100.8095

				118.13		100.8095

				118.15		100.8095

				118.18		100.8095

				118.2		100.8095

				118.22		100.8095

				118.24		100.8095

				118.26		100.8095

				118.28		100.8095

				118.3		100.8095

				118.32		100.8095

				118.34		100.8095

				118.37		100.8095

				118.39		100.8095

				118.41		100.8095

				118.43		100.8095

				118.45		100.8095

				118.47		100.8095

				118.49		100.8095

				118.51		100.8095

				118.53		100.8095

				118.55		100.8095

				118.58		100.8095

				118.6		100.8095

				118.62		100.8095

				118.64		100.8095

				118.66		100.8095

				118.68		100.8095

				118.7		100.8095

				118.72		100.8095

				118.74		100.8095

				118.76		100.8095

				118.79		100.8095

				118.81		100.8095

				118.83		100.8095

				118.85		100.8095

				118.87		100.8051

				118.89		100.8095

				118.91		100.8095

				118.93		100.8095

				118.95		100.8095

				118.97		100.8095

				119		100.8095

				119.02		100.8051

				119.04		100.8051

				119.06		100.8051

				119.08		100.8051

				119.1		100.8051

				119.12		100.8051

				119.14		100.8051

				119.16		100.8051

				119.18		100.8051

				119.21		100.8051

				119.23		100.8051

				119.25		100.8051

				119.27		100.8051

				119.29		100.8051

				119.31		100.8051

				119.33		100.8051

				119.35		100.8051

				119.37		100.8051

				119.39		100.8051

				119.42		100.8051

				119.44		100.8051

				119.46		100.8051

				119.48		100.8051

				119.5		100.8051

				119.52		100.8051

				119.54		100.8051

				119.56		100.8051

				119.58		100.8051

				119.6		100.8051

				119.62		100.8051

				119.65		100.8007

				119.67		100.8051

				119.69		100.8051

				119.71		100.8051

				119.73		100.8051

				119.75		100.8051

				119.77		100.8051

				119.79		100.8051

				119.81		100.8051

				119.84		100.8051

				119.86		100.8051

				119.88		100.8051

				119.9		100.8007

				119.92		100.8051

				119.94		100.8051

				119.96		100.8007

				119.98		100.8007

				120		100.8007

				120.02		100.8007

				120.05		100.8007

				120.07		100.8007

				120.09		100.8007

				120.11		100.8007

				120.13		100.8007

				120.15		100.8007

				120.17		100.8007

				120.19		100.8007

				120.21		100.8007

				120.23		100.8007

				120.26		100.8007

				120.28		100.8007

				120.3		100.8007

				120.32		100.8007

				120.34		100.8007

				120.36		100.8007

				120.38		100.8007

				120.4		100.8007

				120.42		100.8007

				120.44		100.8007

				120.47		100.8007

				120.49		100.8007

				120.51		100.8007

				120.53		100.8007

				120.55		100.8007

				120.57		100.8007

				120.59		100.7963

				120.61		100.7963

				120.63		100.7963

				120.65		100.7963

				120.68		100.7963

				120.7		100.7963

				120.72		100.8007

				120.74		100.8007

				120.76		100.8007

				120.78		100.8007

				120.8		100.8007

				120.82		100.8007

				120.84		100.8007

				120.86		100.8007

				120.89		100.8007

				120.91		100.8007

				120.93		100.8007

				120.95		100.8007

				120.97		100.8007

				120.99		100.8007

				121.01		100.8007

				121.03		100.8007

				121.05		100.8007

				121.07		100.8007

				121.1		100.8007

				121.12		100.8007

				121.14		100.8007

				121.16		100.8007

				121.18		100.8007

				121.2		100.8007

				121.22		100.8007

				121.24		100.8007

				121.26		100.8007

				121.28		100.8007

				121.31		100.8007

				121.33		100.8007

				121.35		100.8007

				121.37		100.8007

				121.39		100.8007

				121.41		100.8007

				121.43		100.8007

				121.45		100.8007

				121.47		100.8007

				121.49		100.8007

				121.52		100.8007

				121.54		100.8007

				121.56		100.8007

				121.58		100.8007

				121.6		100.8007

				121.62		100.8007

				121.64		100.8007

				121.66		100.8007

				121.68		100.8007

				121.7		100.8007

				121.73		100.8007

				121.75		100.8007

				121.77		100.8007

				121.79		100.8007

				121.81		100.8007

				121.83		100.8007

				121.85		100.8007

				121.87		100.8007

				121.89		100.8007

				121.91		100.8007

				121.94		100.8007

				121.96		100.8007

				121.98		100.8007

				122		100.8007

				122.02		100.8007

				122.04		100.8007

				122.06		100.8007

				122.08		100.8007

				122.1		100.8007

				122.12		100.8007

				122.15		100.8007

				122.17		100.8007

				122.19		100.8007

				122.21		100.8007

				122.23		100.8007

				122.25		100.8007

				122.27		100.8007

				122.29		100.8007

				122.31		100.8007

				122.33		100.8007

				122.36		100.8007

				122.38		100.8007

				122.4		100.8007

				122.42		100.8007

				122.44		100.8007

				122.46		100.8007

				122.48		100.8007

				122.5		100.8007

				122.52		100.8007

				122.54		100.8007

				122.57		100.8007

				122.59		100.8007

				122.61		100.8007

				122.63		100.8007

				122.65		100.8007

				122.67		100.8007

				122.69		100.8007

				122.71		100.8007

				122.73		100.8007

				122.75		100.8007

				122.78		100.8007

				122.8		100.8007

				122.82		100.8007

				122.84		100.8007

				122.86		100.8007

				122.88		100.8007

				122.9		100.8007

				122.92		100.8007

				122.94		100.8007

				122.96		100.8007

				122.99		100.8007

				123.01		100.8007

				123.03		100.8007

				123.05		100.8007

				123.07		100.8007

				123.09		100.8007

				123.11		100.8007

				123.13		100.8007

				123.15		100.8007

				123.17		100.8007

				123.2		100.8007

				123.22		100.8007

				123.24		100.8007

				123.26		100.8007

				123.28		100.8007

				123.3		100.8007

				123.32		100.8007

				123.34		100.7963

				123.36		100.7963

				123.39		100.7963

				123.41		100.7963

				123.43		100.7963

				123.45		100.7963

				123.47		100.7963

				123.49		100.7963

				123.51		100.7963

				123.53		100.7963

				123.55		100.7963

				123.57		100.7963

				123.6		100.7963

				123.62		100.7963

				123.64		100.7963

				123.66		100.7963

				123.68		100.7963

				123.7		100.7919

				123.72		100.7919

				123.74		100.7963

				123.76		100.7919

				123.79		100.7919

				123.81		100.7919

				123.83		100.7919

				123.85		100.7919

				123.87		100.7919

				123.89		100.7919

				123.91		100.7919

				123.93		100.7919

				123.95		100.7919

				123.97		100.7919

				124		100.7919

				124.02		100.7919

				124.04		100.7919

				124.06		100.7919

				124.08		100.7919

				124.1		100.7919

				124.12		100.7919

				124.14		100.7919

				124.16		100.7919

				124.18		100.7919

				124.21		100.7919

				124.23		100.7919

				124.25		100.7919

				124.27		100.7875

				124.29		100.7875

				124.31		100.7875

				124.33		100.7875

				124.35		100.7875

				124.37		100.7875

				124.4		100.7875

				124.42		100.7875

				124.44		100.7875

				124.46		100.7875

				124.48		100.7875

				124.5		100.7875

				124.52		100.7875

				124.54		100.7875

				124.56		100.7831

				124.58		100.7831

				124.61		100.7831

				124.63		100.7831

				124.65		100.7831

				124.67		100.7831

				124.69		100.7831

				124.71		100.7831

				124.73		100.7831

				124.75		100.7831

				124.77		100.7831

				124.79		100.7787

				124.82		100.7787

				124.84		100.7831

				124.86		100.7787

				124.88		100.7787

				124.9		100.7787

				124.92		100.7787

				124.94		100.7787

				124.96		100.7787

				124.98		100.7787

				125.01		100.7787

				125.03		100.7787

				125.05		100.7743

				125.07		100.7743

				125.09		100.7743

				125.11		100.7743

				125.13		100.7743

				125.15		100.7743

				125.17		100.7743

				125.19		100.7743

				125.22		100.7743

				125.24		100.7743

				125.26		100.7743

				125.28		100.7743

				125.3		100.7743

				125.32		100.7743

				125.34		100.7743

				125.36		100.7743

				125.38		100.7743

				125.4		100.7743

				125.43		100.7743

				125.45		100.7743

				125.47		100.7743

				125.49		100.7743

				125.51		100.7743

				125.53		100.7743

				125.55		100.7743

				125.57		100.7743

				125.59		100.7743

				125.62		100.7743

				125.64		100.7743

				125.66		100.7743

				125.68		100.7743

				125.7		100.7699

				125.72		100.7699

				125.74		100.7699

				125.76		100.7699

				125.78		100.7699

				125.8		100.7699

				125.83		100.7699

				125.85		100.7699

				125.87		100.7699

				125.89		100.7699

				125.91		100.7699

				125.93		100.7699

				125.95		100.7699

				125.97		100.7699

				125.99		100.7699

				126.02		100.7699

				126.04		100.7699

				126.06		100.7655

				126.08		100.7699

				126.1		100.7699

				126.12		100.7699

				126.14		100.7699

				126.16		100.7699

				126.18		100.7655

				126.21		100.7655

				126.23		100.7655

				126.25		100.7655

				126.27		100.7655

				126.29		100.7655

				126.31		100.7655

				126.33		100.7655

				126.35		100.7655

				126.37		100.7655

				126.39		100.7655

				126.42		100.7655

				126.44		100.7655

				126.46		100.7655

				126.48		100.7611

				126.5		100.7611

				126.52		100.7611

				126.54		100.7611

				126.56		100.7611

				126.58		100.7611

				126.61		100.7611

				126.63		100.7611

				126.65		100.7611

				126.67		100.7611

				126.69		100.7611

				126.71		100.7611

				126.73		100.7611

				126.75		100.7611

				126.77		100.7611

				126.8		100.7611

				126.82		100.7611

				126.84		100.7611

				126.86		100.7611

				126.88		100.7611

				126.9		100.7611

				126.92		100.7611

				126.94		100.7611

				126.96		100.7611

				126.98		100.7611

				127.01		100.7567

				127.03		100.7567

				127.05		100.7567

				127.07		100.7567

				127.09		100.7567

				127.11		100.7567

				127.13		100.7567

				127.15		100.7567

				127.17		100.7567

				127.2		100.7567

				127.22		100.7567

				127.24		100.7567

				127.26		100.7567

				127.28		100.7567

				127.3		100.7567

				127.32		100.7567

				127.34		100.7567

				127.36		100.7567

				127.39		100.7567

				127.41		100.7567

				127.43		100.7567

				127.45		100.7567

				127.47		100.7567

				127.49		100.7567

				127.51		100.7567

				127.53		100.7567

				127.55		100.7567

				127.57		100.7567

				127.6		100.7567

				127.62		100.7567

				127.64		100.7567

				127.66		100.7567

				127.68		100.7567

				127.7		100.7523

				127.72		100.7567

				127.74		100.7567

				127.76		100.7567

				127.79		100.7567

				127.81		100.7567

				127.83		100.7567

				127.85		100.7567

				127.87		100.7523

				127.89		100.7567

				127.91		100.7523

				127.93		100.7523

				127.95		100.7523

				127.98		100.7523

				128		100.7523

				128.02		100.7523

				128.04		100.7523

				128.06		100.7523

				128.08		100.7523

				128.1		100.7523

				128.12		100.7523

				128.14		100.7523

				128.16		100.7523

				128.19		100.7523

				128.21		100.7523

				128.23		100.7523

				128.25		100.7523

				128.27		100.7523

				128.29		100.7523

				128.31		100.7523

				128.33		100.7523

				128.35		100.7523

				128.38		100.7523

				128.4		100.7523

				128.42		100.7523

				128.44		100.7523

				128.46		100.7523

				128.48		100.7523

				128.5		100.7523

				128.52		100.7523

				128.54		100.7523

				128.57		100.7523

				128.59		100.7523

				128.61		100.7523

				128.63		100.7523

				128.65		100.7523

				128.67		100.7523

				128.69		100.7523

				128.71		100.7523

				128.73		100.7523

				128.75		100.7523

				128.78		100.7523

				128.8		100.7523

				128.82		100.7523

				128.84		100.7523

				128.86		100.7523

				128.88		100.7479

				128.9		100.7479

				128.92		100.7479

				128.94		100.7479

				128.97		100.7479

				128.99		100.7479

				129.01		100.7479

				129.03		100.7479

				129.05		100.7479

				129.07		100.7479

				129.09		100.7479

				129.11		100.7479

				129.13		100.7435

				129.16		100.7479

				129.18		100.7435

				129.2		100.7435

				129.22		100.7435

				129.24		100.7435

				129.26		100.7435

				129.28		100.7435

				129.3		100.7435

				129.32		100.7435

				129.35		100.7435

				129.37		100.7435

				129.39		100.7435

				129.41		100.7435

				129.43		100.7391

				129.45		100.7391

				129.47		100.7391

				129.49		100.7391

				129.51		100.7391

				129.54		100.7391

				129.56		100.7391

				129.58		100.7391

				129.6		100.7391

				129.62		100.7391

				129.64		100.7391

				129.66		100.7391

				129.68		100.7391

				129.7		100.7391

				129.73		100.7391

				129.75		100.7391

				129.77		100.7391

				129.79		100.7347

				129.81		100.7347

				129.83		100.7347

				129.85		100.7347

				129.87		100.7347

				129.89		100.7347

				129.92		100.7347

				129.94		100.7347

				129.96		100.7347

				129.98		100.7347

				130		100.7347

				130.02		100.7347

				130.04		100.7347

				130.06		100.7303

				130.08		100.7303

				130.11		100.7303

				130.13		100.7303

				130.15		100.7303

				130.17		100.7303

				130.19		100.7303

				130.21		100.7303

				130.23		100.7303

				130.25		100.7303

				130.27		100.7303

				130.3		100.7303

				130.32		100.7303

				130.34		100.7303

				130.36		100.7303

				130.38		100.7303

				130.4		100.7259

				130.42		100.7259

				130.44		100.7259

				130.46		100.7259

				130.49		100.7259

				130.51		100.7259

				130.53		100.7259

				130.55		100.7259

				130.57		100.7259

				130.59		100.7259

				130.61		100.7259

				130.63		100.7259

				130.65		100.7259

				130.68		100.7259

				130.7		100.7259

				130.72		100.7259

				130.74		100.7259

				130.76		100.7259

				130.78		100.7259

				130.8		100.7259

				130.82		100.7259

				130.84		100.7259

				130.87		100.7215

				130.89		100.7215

				130.91		100.7215

				130.93		100.7215

				130.95		100.7215

				130.97		100.7215

				130.99		100.7215

				131.01		100.7215

				131.03		100.7215

				131.06		100.7215

				131.08		100.7215

				131.1		100.7215

				131.12		100.7215

				131.14		100.7215

				131.16		100.7215

				131.18		100.7215

				131.2		100.7215

				131.22		100.7171

				131.25		100.7171

				131.27		100.7171

				131.29		100.7171

				131.31		100.7171

				131.33		100.7171

				131.35		100.7171

				131.37		100.7171

				131.39		100.7171

				131.41		100.7171

				131.44		100.7171

				131.46		100.7171

				131.48		100.7171

				131.5		100.7171

				131.52		100.7171

				131.54		100.7127

				131.56		100.7127

				131.58		100.7127

				131.6		100.7127

				131.63		100.7127

				131.65		100.7127

				131.67		100.7127

				131.69		100.7127

				131.71		100.7127

				131.73		100.7083

				131.75		100.7083

				131.77		100.7083

				131.79		100.7083

				131.82		100.7083

				131.84		100.7083

				131.86		100.7083

				131.88		100.7083

				131.9		100.7083

				131.92		100.7083

				131.94		100.7039

				131.96		100.7039

				131.99		100.7039

				132.01		100.7039

				132.03		100.7039

				132.05		100.7039

				132.07		100.7039

				132.09		100.7039

				132.11		100.7039

				132.13		100.7039

				132.15		100.7039

				132.18		100.7039

				132.2		100.6995

				132.22		100.6995

				132.24		100.6995

				132.26		100.6995

				132.28		100.6995

				132.3		100.6995

				132.32		100.6995

				132.34		100.6995

				132.37		100.6995

				132.39		100.6995

				132.41		100.6995

				132.43		100.6995

				132.45		100.6995

				132.47		100.6951

				132.49		100.6951

				132.51		100.6951

				132.53		100.6951

				132.56		100.6951

				132.58		100.6951

				132.6		100.6951

				132.62		100.6951

				132.64		100.6951

				132.66		100.6951

				132.68		100.6951

				132.7		100.6951

				132.72		100.6951

				132.75		100.6907

				132.77		100.6907

				132.79		100.6907

				132.81		100.6907

				132.83		100.6907

				132.85		100.6907

				132.87		100.6907

				132.89		100.6907

				132.91		100.6907

				132.94		100.6907

				132.96		100.6863

				132.98		100.6863

				133		100.6863

				133.02		100.6863

				133.04		100.6863

				133.06		100.6863

				133.08		100.6863

				133.1		100.6863

				133.13		100.6863

				133.15		100.6863

				133.17		100.6863

				133.19		100.6863

				133.21		100.6819

				133.23		100.6819

				133.25		100.6819

				133.27		100.6819

				133.3		100.6819

				133.32		100.6819

				133.34		100.6819

				133.36		100.6819

				133.38		100.6819

				133.4		100.6819

				133.42		100.6819

				133.44		100.6819

				133.46		100.6819

				133.49		100.6819

				133.51		100.6819

				133.53		100.6819

				133.55		100.6775

				133.57		100.6775

				133.59		100.6775

				133.61		100.6775

				133.63		100.6775

				133.65		100.6775

				133.68		100.6775

				133.7		100.6775

				133.72		100.6775

				133.74		100.6775

				133.76		100.6775

				133.78		100.6775

				133.8		100.6775

				133.82		100.6775

				133.84		100.6775

				133.87		100.6775

				133.89		100.6775

				133.91		100.6775

				133.93		100.6775

				133.95		100.6731

				133.97		100.6731

				133.99		100.6731

				134.01		100.6731

				134.03		100.6731

				134.06		100.6731

				134.08		100.6731

				134.1		100.6731

				134.12		100.6731

				134.14		100.6731

				134.16		100.6731

				134.18		100.6731

				134.2		100.6731

				134.22		100.6731

				134.25		100.6731

				134.27		100.6731

				134.29		100.6731

				134.31		100.6687

				134.33		100.6731

				134.35		100.6687

				134.37		100.6687

				134.39		100.6687

				134.42		100.6687

				134.44		100.6687

				134.46		100.6687

				134.48		100.6687

				134.5		100.6687

				134.52		100.6687

				134.54		100.6643

				134.56		100.6643

				134.58		100.6643

				134.61		100.6643

				134.63		100.6643

				134.65		100.6643

				134.67		100.6643

				134.69		100.6643

				134.71		100.6643

				134.73		100.6599

				134.75		100.6599

				134.77		100.6599

				134.8		100.6599

				134.82		100.6599

				134.84		100.6599

				134.86		100.6599

				134.88		100.6599

				134.9		100.6599

				134.92		100.6599

				134.94		100.6599

				134.97		100.6599

				134.99		100.6599

				135.01		100.6599

				135.03		100.6555

				135.05		100.6555

				135.07		100.6555

				135.09		100.6555

				135.11		100.6555

				135.13		100.6555

				135.16		100.6555

				135.18		100.6555

				135.2		100.6555

				135.22		100.6555

				135.24		100.6555

				135.26		100.6555

				135.28		100.6511

				135.3		100.6511

				135.32		100.6511

				135.35		100.6511

				135.37		100.6511

				135.39		100.6511

				135.41		100.6511

				135.43		100.6511

				135.45		100.6511

				135.47		100.6511

				135.49		100.6511

				135.52		100.6511

				135.54		100.6467

				135.56		100.6467

				135.58		100.6467

				135.6		100.6467

				135.62		100.6467

				135.64		100.6467

				135.66		100.6467

				135.68		100.6467

				135.71		100.6467

				135.73		100.6467

				135.75		100.6467

				135.77		100.6467

				135.79		100.6467

				135.81		100.6467

				135.83		100.6467

				135.85		100.6467

				135.88		100.6467

				135.9		100.6467

				135.92		100.6467

				135.94		100.6423

				135.96		100.6423

				135.98		100.6423

				136		100.6423

				136.02		100.6423

				136.04		100.6423

				136.07		100.6423

				136.09		100.6423

				136.11		100.6423

				136.13		100.6423

				136.15		100.6379

				136.17		100.6379

				136.19		100.6379

				136.21		100.6379

				136.23		100.6379

				136.26		100.6379

				136.28		100.6379

				136.3		100.6335

				136.32		100.6335

				136.34		100.6335

				136.36		100.6335

				136.38		100.6335

				136.4		100.6335

				136.43		100.6335

				136.45		100.6335

				136.47		100.6291

				136.49		100.6291

				136.51		100.6291

				136.53		100.6291

				136.55		100.6291

				136.57		100.6291

				136.59		100.6291

				136.62		100.6291

				136.64		100.6291

				136.66		100.6291

				136.68		100.6291

				136.7		100.6291

				136.72		100.6291

				136.74		100.6247

				136.76		100.6247

				136.78		100.6247

				136.81		100.6247

				136.83		100.6247

				136.85		100.6247

				136.87		100.6247

				136.89		100.6247

				136.91		100.6247

				136.93		100.6247

				136.95		100.6203

				136.98		100.6203

				137		100.6203

				137.02		100.6203

				137.04		100.6203

				137.06		100.6203

				137.08		100.6203

				137.1		100.6203

				137.12		100.6203

				137.14		100.6203

				137.17		100.6203

				137.19		100.6203

				137.21		100.6159

				137.23		100.6159

				137.25		100.6159

				137.27		100.6159

				137.29		100.6159

				137.31		100.6159

				137.33		100.6159

				137.36		100.6159

				137.38		100.6159

				137.4		100.6159

				137.42		100.6159

				137.44		100.6115

				137.46		100.6115

				137.48		100.6115

				137.5		100.6115

				137.52		100.6115

				137.55		100.6115

				137.57		100.6115

				137.59		100.6115

				137.61		100.6115

				137.63		100.6071

				137.65		100.6071

				137.67		100.6071

				137.69		100.6071

				137.72		100.6071

				137.74		100.6071

				137.76		100.6071

				137.78		100.6071

				137.8		100.6071

				137.82		100.6071

				137.84		100.6027

				137.86		100.6027

				137.88		100.6027

				137.91		100.6027

				137.93		100.6027

				137.95		100.6027

				137.97		100.6027

				137.99		100.5983

				138.01		100.5983

				138.03		100.5983

				138.05		100.5983

				138.07		100.5983

				138.1		100.5983

				138.12		100.5983

				138.14		100.5939

				138.16		100.5939

				138.18		100.5939

				138.2		100.5939

				138.22		100.5939

				138.24		100.5939

				138.27		100.5939

				138.29		100.5939

				138.31		100.5939

				138.33		100.5939

				138.35		100.5939

				138.37		100.5939

				138.39		100.5939

				138.41		100.5939

				138.43		100.5895

				138.46		100.5895

				138.48		100.5895

				138.5		100.5895

				138.52		100.5895

				138.54		100.5895

				138.56		100.5895

				138.58		100.5895

				138.6		100.5895

				138.62		100.5895

				138.65		100.5851

				138.67		100.5851

				138.69		100.5851

				138.71		100.5851

				138.73		100.5851

				138.75		100.5851

				138.77		100.5851

				138.79		100.5851

				138.82		100.5851

				138.84		100.5851

				138.86		100.5851

				138.88		100.5851

				138.9		100.5807

				138.92		100.5807

				138.94		100.5807

				138.96		100.5807

				138.98		100.5807

				139.01		100.5807

				139.03		100.5807

				139.05		100.5807

				139.07		100.5807

				139.09		100.5807

				139.11		100.5807

				139.13		100.5763

				139.15		100.5763

				139.18		100.5763

				139.2		100.5763

				139.22		100.5763

				139.24		100.5763

				139.26		100.5763

				139.28		100.5719

				139.3		100.5719

				139.32		100.5719

				139.34		100.5719

				139.37		100.5719

				139.39		100.5719

				139.41		100.5719

				139.43		100.5719

				139.45		100.5719

				139.47		100.5719

				139.49		100.5675

				139.51		100.5675

				139.54		100.5675

				139.56		100.5675

				139.58		100.5675

				139.6		100.5675

				139.62		100.5631

				139.64		100.5631

				139.66		100.5631

				139.68		100.5631

				139.7		100.5631

				139.73		100.5631

				139.75		100.5631

				139.77		100.5631

				139.79		100.5587

				139.81		100.5587

				139.83		100.5587

				139.85		100.5587

				139.87		100.5587

				139.9		100.5587

				139.92		100.5587

				139.94		100.5587

				139.96		100.5587

				139.98		100.5587

				140		100.5543

				140.02		100.5543

				140.04		100.5543

				140.06		100.5543

				140.09		100.5543

				140.11		100.5543

				140.13		100.5543

				140.15		100.5543

				140.17		100.5543

				140.19		100.5543

				140.21		100.5543

				140.23		100.5543

				140.26		100.5543

				140.28		100.5499

				140.3		100.5499

				140.32		100.5499

				140.34		100.5499

				140.36		100.5499

				140.38		100.5499

				140.4		100.5499

				140.42		100.5499

				140.45		100.5499

				140.47		100.5499

				140.49		100.5455

				140.51		100.5455

				140.53		100.5455

				140.55		100.5455

				140.57		100.5455

				140.59		100.5455

				140.61		100.5455

				140.64		100.5455

				140.66		100.5455

				140.68		100.5411

				140.7		100.5411

				140.72		100.5411

				140.74		100.5411

				140.76		100.5411

				140.78		100.5411

				140.81		100.5411

				140.83		100.5411

				140.85		100.5411

				140.87		100.5367

				140.89		100.5367

				140.91		100.5367

				140.93		100.5367

				140.95		100.5367

				140.97		100.5367

				141		100.5367

				141.02		100.5323

				141.04		100.5323

				141.06		100.5323

				141.08		100.5323

				141.1		100.5323

				141.12		100.5323

				141.14		100.5279

				141.17		100.5279

				141.19		100.5279

				141.21		100.5279

				141.23		100.5279

				141.25		100.5279

				141.27		100.5279

				141.29		100.5279

				141.31		100.5279

				141.33		100.5235

				141.36		100.5235

				141.38		100.5235

				141.4		100.5235

				141.42		100.5235

				141.44		100.5235

				141.46		100.5235

				141.48		100.5235

				141.5		100.5235

				141.53		100.5235

				141.55		100.5191

				141.57		100.5191

				141.59		100.5191

				141.61		100.5191

				141.63		100.5191

				141.65		100.5191

				141.67		100.5191

				141.7		100.5147

				141.72		100.5147

				141.74		100.5147

				141.76		100.5147

				141.78		100.5147

				141.8		100.5147

				141.82		100.5103

				141.84		100.5103

				141.86		100.5103

				141.89		100.5103

				141.91		100.5103

				141.93		100.5059

				141.95		100.5059

				141.97		100.5059

				141.99		100.5059

				142.01		100.5059

				142.03		100.5059

				142.06		100.5015

				142.08		100.5015

				142.1		100.5015

				142.12		100.5015

				142.14		100.4971

				142.16		100.4971

				142.18		100.4971

				142.2		100.4971

				142.22		100.4927

				142.25		100.4927

				142.27		100.4927

				142.29		100.4927

				142.31		100.4883

				142.33		100.4883

				142.35		100.4883

				142.37		100.4883

				142.39		100.4883

				142.41		100.4883

				142.44		100.4883

				142.46		100.4839

				142.48		100.4839

				142.5		100.4839

				142.52		100.4839

				142.54		100.4795

				142.56		100.4795

				142.58		100.4795

				142.61		100.4795

				142.63		100.4795

				142.65		100.4751

				142.67		100.4751

				142.69		100.4751

				142.71		100.4751

				142.73		100.4751

				142.75		100.4751

				142.77		100.4751

				142.8		100.4707

				142.82		100.4707

				142.84		100.4707

				142.86		100.4707

				142.88		100.4707

				142.9		100.4707

				142.92		100.4707

				142.94		100.4663

				142.97		100.4663

				142.99		100.4663

				143.01		100.4663

				143.03		100.4619

				143.05		100.4619

				143.07		100.4619

				143.09		100.4619

				143.11		100.4575

				143.14		100.4619

				143.16		100.4575

				143.18		100.4575

				143.2		100.4575

				143.22		100.4575

				143.24		100.4575

				143.26		100.4531

				143.28		100.4531

				143.3		100.4531

				143.33		100.4531

				143.35		100.4531

				143.37		100.4531

				143.39		100.4487

				143.41		100.4487

				143.43		100.4487

				143.45		100.4487

				143.47		100.4487

				143.5		100.4487

				143.52		100.4487

				143.54		100.4443

				143.56		100.4443

				143.58		100.4443

				143.6		100.4443

				143.62		100.4443

				143.64		100.4443

				143.67		100.4443

				143.69		100.4443

				143.71		100.4399

				143.73		100.4399

				143.75		100.4399

				143.77		100.4399

				143.79		100.4399

				143.81		100.4399

				143.84		100.4355

				143.86		100.4355

				143.88		100.4355

				143.9		100.4355

				143.92		100.4355

				143.94		100.4355

				143.96		100.4355

				143.98		100.4355

				144		100.4311

				144.03		100.4311

				144.05		100.4311

				144.07		100.4311

				144.09		100.4311

				144.11		100.4267

				144.13		100.4267

				144.15		100.4267

				144.17		100.4267

				144.2		100.4267

				144.22		100.4223

				144.24		100.4223

				144.26		100.4223

				144.28		100.4223

				144.3		100.4223

				144.32		100.4179

				144.34		100.4179

				144.36		100.4179

				144.39		100.4179

				144.41		100.4179

				144.43		100.4179

				144.45		100.4135

				144.47		100.4135

				144.49		100.4135

				144.51		100.4135

				144.53		100.4135

				144.56		100.4135

				144.58		100.4091

				144.6		100.4091

				144.62		100.4091

				144.64		100.4091

				144.66		100.4091

				144.68		100.4047

				144.7		100.4047

				144.72		100.4047

				144.75		100.4047

				144.77		100.4003

				144.79		100.4003

				144.81		100.4003

				144.83		100.4003

				144.85		100.4003

				144.87		100.4003

				144.89		100.3959

				144.92		100.3959

				144.94		100.3959

				144.96		100.3959

				144.98		100.3959

				145		100.3959

				145.02		100.3959

				145.04		100.3959

				145.06		100.3915

				145.09		100.3915

				145.11		100.3915

				145.13		100.3915

				145.15		100.3871

				145.17		100.3871

				145.19		100.3871

				145.21		100.3871

				145.23		100.3871

				145.25		100.3871

				145.28		100.3871

				145.3		100.3871

				145.32		100.3871

				145.34		100.3827

				145.36		100.3827

				145.38		100.3827

				145.4		100.3827

				145.42		100.3827

				145.45		100.3783

				145.47		100.3783

				145.49		100.3783

				145.51		100.3783

				145.53		100.3783

				145.55		100.3783

				145.57		100.3739

				145.59		100.3739

				145.62		100.3739

				145.64		100.3739

				145.66		100.3739

				145.68		100.3739

				145.7		100.3739

				145.72		100.3695

				145.74		100.3695

				145.76		100.3695

				145.78		100.3695

				145.81		100.3695

				145.83		100.3695

				145.85		100.3695

				145.87		100.3695

				145.89		100.3651

				145.91		100.3651

				145.93		100.3651

				145.95		100.3651

				145.98		100.3651

				146		100.3651

				146.02		100.3651

				146.04		100.3607

				146.06		100.3607

				146.08		100.3607

				146.1		100.3607

				146.12		100.3607

				146.15		100.3607

				146.17		100.3607

				146.19		100.3607

				146.21		100.3563

				146.23		100.3563

				146.25		100.3563

				146.27		100.3563

				146.29		100.3563

				146.32		100.3563

				146.34		100.3519

				146.36		100.3563

				146.38		100.3519

				146.4		100.3519

				146.42		100.3519

				146.44		100.3519

				146.46		100.3519

				146.48		100.3475

				146.51		100.3475

				146.53		100.3475

				146.55		100.3475

				146.57		100.3475

				146.59		100.3431

				146.61		100.3431

				146.63		100.3431

				146.65		100.3431

				146.68		100.3431

				146.7		100.3431

				146.72		100.3431

				146.74		100.3387

				146.76		100.3387

				146.78		100.3387

				146.8		100.3387

				146.82		100.3387

				146.85		100.3387

				146.87		100.3343

				146.89		100.3343

				146.91		100.3343

				146.93		100.3343

				146.95		100.3299

				146.97		100.3299

				146.99		100.3299

				147.01		100.3299

				147.04		100.3299

				147.06		100.3299

				147.08		100.3255

				147.1		100.3255

				147.12		100.3255

				147.14		100.3211

				147.16		100.3211

				147.18		100.3211

				147.21		100.3211

				147.23		100.3167

				147.25		100.3167

				147.27		100.3167

				147.29		100.3167

				147.31		100.3167

				147.33		100.3123

				147.35		100.3123

				147.37		100.3123

				147.4		100.3123

				147.42		100.3079

				147.44		100.3079

				147.46		100.3079

				147.48		100.3079

				147.5		100.3079

				147.52		100.3036

				147.54		100.3036

				147.57		100.3036

				147.59		100.2992

				147.61		100.2992

				147.63		100.2992

				147.65		100.2948

				147.67		100.2948

				147.69		100.2948

				147.71		100.2948

				147.74		100.2948

				147.76		100.2904

				147.78		100.2904

				147.8		100.286

				147.82		100.286

				147.84		100.286

				147.86		100.286

				147.88		100.286

				147.9		100.2816

				147.93		100.2816

				147.95		100.2816

				147.97		100.2772

				147.99		100.2772

				148.01		100.2772

				148.03		100.2772

				148.05		100.2772

				148.07		100.2728

				148.1		100.2728

				148.12		100.2728

				148.14		100.2728

				148.16		100.2684

				148.18		100.2684

				148.2		100.2684

				148.22		100.2684

				148.24		100.264

				148.26		100.264

				148.29		100.264

				148.31		100.264

				148.33		100.264

				148.35		100.2596

				148.37		100.2596

				148.39		100.2596

				148.41		100.2596

				148.43		100.2596

				148.46		100.2596

				148.48		100.2552

				148.5		100.2552

				148.52		100.2552

				148.54		100.2508

				148.56		100.2508

				148.58		100.2508

				148.6		100.2508

				148.63		100.2508

				148.65		100.2464

				148.67		100.2464

				148.69		100.2464

				148.71		100.242

				148.73		100.242

				148.75		100.242

				148.77		100.242

				148.79		100.2376

				148.82		100.2376

				148.84		100.2376

				148.86		100.2376

				148.88		100.2376

				148.9		100.2376

				148.92		100.2376

				148.94		100.2332

				148.96		100.2332

				148.99		100.2332

				149.01		100.2288

				149.03		100.2288

				149.05		100.2288

				149.07		100.2288

				149.09		100.2288

				149.11		100.2288

				149.13		100.2288

				149.16		100.2288

				149.18		100.2244

				149.2		100.2244

				149.22		100.2244

				149.24		100.22

				149.26		100.22

				149.28		100.22

				149.3		100.22

				149.33		100.22

				149.35		100.22

				149.37		100.2156

				149.39		100.2156

				149.41		100.2156

				149.43		100.2156

				149.45		100.2112

				149.47		100.2112

				149.49		100.2112

				149.52		100.2112

				149.54		100.2112

				149.56		100.2068

				149.58		100.2068

				149.6		100.2068

				149.62		100.2068

				149.64		100.2068

				149.66		100.2024

				149.69		100.2024

				149.71		100.2024

				149.73		100.2024

				149.75		100.2024

				149.77		100.2024

				149.79		100.198

				149.81		100.198

				149.83		100.198

				149.86		100.198

				149.88		100.198

				149.9		100.198

				149.92		100.1936

				149.94		100.1936

				149.96		100.1936

				149.98		100.1936

				150		100.1892

				150.03		100.1892

				150.05		100.1892

				150.07		100.1892

				150.09		100.1848

				150.11		100.1848

				150.13		100.1804

				150.15		100.1804

				150.17		100.1804

				150.2		100.176

				150.22		100.176

				150.24		100.176

				150.26		100.176

				150.28		100.176

				150.3		100.1716

				150.32		100.1716

				150.34		100.1716

				150.36		100.1716

				150.39		100.1672

				150.41		100.1672

				150.43		100.1672

				150.45		100.1628

				150.47		100.1628

				150.49		100.1628

				150.51		100.1584

				150.53		100.1584

				150.56		100.1584

				150.58		100.154

				150.6		100.1584

				150.62		100.154

				150.64		100.154

				150.66		100.1496

				150.68		100.1496

				150.7		100.1452

				150.73		100.1452

				150.75		100.1452

				150.77		100.1452

				150.79		100.1408

				150.81		100.1408

				150.83		100.1364

				150.85		100.1364

				150.87		100.1364

				150.89		100.1364

				150.92		100.132

				150.94		100.132

				150.96		100.132

				150.98		100.132

				151		100.1276

				151.02		100.1276

				151.04		100.1276

				151.06		100.1276

				151.09		100.1276

				151.11		100.1232

				151.13		100.1232

				151.15		100.1232

				151.17		100.1188

				151.19		100.1188

				151.21		100.1188

				151.23		100.1188

				151.26		100.1144

				151.28		100.1144

				151.3		100.11

				151.32		100.11

				151.34		100.11

				151.36		100.1056

				151.38		100.1056

				151.4		100.1056

				151.43		100.1012

				151.45		100.1012

				151.47		100.1012

				151.49		100.1012

				151.51		100.1012

				151.53		100.0968

				151.55		100.0968

				151.57		100.0968

				151.59		100.0968

				151.62		100.0924

				151.64		100.0924

				151.66		100.0924

				151.68		100.0924

				151.7		100.088

				151.72		100.088

				151.74		100.088

				151.76		100.0836

				151.79		100.0836

				151.81		100.0792

				151.83		100.0792

				151.85		100.0748

				151.87		100.0748

				151.89		100.0748

				151.91		100.0748

				151.93		100.0704

				151.96		100.0704

				151.98		100.0704

				152		100.066

				152.02		100.066

				152.04		100.066

				152.06		100.066

				152.08		100.066

				152.1		100.0616

				152.13		100.0616

				152.15		100.0616

				152.17		100.0616

				152.19		100.0572

				152.21		100.0572

				152.23		100.0572

				152.25		100.0572

				152.27		100.0528

				152.3		100.0528

				152.32		100.0528

				152.34		100.0528

				152.36		100.0484

				152.38		100.0484

				152.4		100.0484

				152.42		100.0484

				152.44		100.044

				152.46		100.044

				152.49		100.044

				152.51		100.0396

				152.53		100.0396

				152.55		100.0396

				152.57		100.0396

				152.59		100.0396

				152.61		100.0396

				152.63		100.0352

				152.66		100.0352

				152.68		100.0352

				152.7		100.0352

				152.72		100.0308

				152.74		100.0308

				152.76		100.0308

				152.78		100.0264

				152.8		100.0264

				152.83		100.0264

				152.85		100.022

				152.87		100.022

				152.89		100.022

				152.91		100.0176

				152.93		100.0176

				152.95		100.0176

				152.97		100.0132

				152.99		100.0132

				153.02		100.0132

				153.04		100.0088

				153.06		100.0088

				153.08		100.0088

				153.1		100.0044

				153.12		100.0044

				153.14		100

				153.16		100

				153.19		99.9956

				153.21		99.9956

				153.23		99.9956

				153.25		99.9912

				153.27		99.9912

				153.29		99.9912

				153.31		99.9912

				153.33		99.9868

				153.35		99.9868

				153.38		99.9868

				153.4		99.9824

				153.42		99.9824

				153.44		99.978

				153.46		99.9824

				153.48		99.978

				153.5		99.978

				153.52		99.9736

				153.55		99.9736

				153.57		99.9736

				153.59		99.9736

				153.61		99.96921

				153.63		99.96921

				153.65		99.96921

				153.67		99.96921

				153.69		99.96481

				153.71		99.96481

				153.74		99.96481

				153.76		99.96481

				153.78		99.96041

				153.8		99.96041

				153.82		99.96041

				153.84		99.95601

				153.86		99.95601

				153.88		99.95601

				153.9		99.95601

				153.93		99.95601

				153.95		99.95601

				153.97		99.95601

				153.99		99.95161

				154.01		99.95161

				154.03		99.95161

				154.05		99.95161

				154.07		99.94721

				154.1		99.94721

				154.12		99.94721

				154.14		99.94281

				154.16		99.94281

				154.18		99.94281

				154.2		99.93841

				154.22		99.93841

				154.24		99.93401

				154.26		99.93401

				154.29		99.93401

				154.31		99.93401

				154.33		99.92961

				154.35		99.92961

				154.37		99.92961

				154.39		99.92961

				154.41		99.92961

				154.43		99.92521

				154.46		99.92521

				154.48		99.92081

				154.5		99.92081

				154.52		99.91641

				154.54		99.91641

				154.56		99.91641

				154.58		99.91201

				154.6		99.91201

				154.62		99.90762

				154.65		99.90762

				154.67		99.90322

				154.69		99.90322

				154.71		99.90322

				154.73		99.90322

				154.75		99.89882

				154.77		99.89882

				154.79		99.89442

				154.81		99.89442

				154.84		99.89442

				154.86		99.89442

				154.88		99.89002

				154.9		99.89002

				154.92		99.88562

				154.94		99.88562

				154.96		99.88562

				154.98		99.88562

				155.01		99.88122

				155.03		99.88122

				155.05		99.87682

				155.07		99.87682

				155.09		99.87242

				155.11		99.87242

				155.13		99.86802

				155.15		99.86802

				155.17		99.86802

				155.2		99.86362

				155.22		99.86362

				155.24		99.86362

				155.26		99.85922

				155.28		99.85922

				155.3		99.85922

				155.32		99.85482

				155.34		99.85482

				155.36		99.85482

				155.39		99.85042

				155.41		99.85042

				155.43		99.84603

				155.45		99.84603

				155.47		99.84603

				155.49		99.84163

				155.51		99.83723

				155.53		99.84163

				155.56		99.83723

				155.58		99.83723

				155.6		99.83283

				155.62		99.83283

				155.64		99.82843

				155.66		99.82843

				155.68		99.82403

				155.7		99.82403

				155.72		99.82403

				155.75		99.81963

				155.77		99.81963

				155.79		99.81963

				155.81		99.81523

				155.83		99.81523

				155.85		99.81523

				155.87		99.81083

				155.89		99.81083

				155.91		99.80643

				155.94		99.80643

				155.96		99.80203

				155.98		99.80203

				156		99.80203

				156.02		99.79763

				156.04		99.79763

				156.06		99.79323

				156.08		99.79323

				156.11		99.79323

				156.13		99.78883

				156.15		99.78883

				156.17		99.78883

				156.19		99.78444

				156.21		99.78444

				156.23		99.78004

				156.25		99.78004

				156.27		99.78004

				156.3		99.78004

				156.32		99.77564

				156.34		99.77564

				156.36		99.77124

				156.38		99.77124

				156.4		99.77124

				156.42		99.77124

				156.44		99.77124

				156.46		99.76684

				156.49		99.76684

				156.51		99.76684

				156.53		99.76244

				156.55		99.76244

				156.57		99.76244

				156.59		99.75804

				156.61		99.75804

				156.63		99.75364

				156.66		99.75364

				156.68		99.75364

				156.7		99.74924

				156.72		99.74924

				156.74		99.74924

				156.76		99.74484

				156.78		99.74484

				156.8		99.74484

				156.82		99.74044

				156.85		99.74044

				156.87		99.74044

				156.89		99.74044

				156.91		99.73604

				156.93		99.73604

				156.95		99.73604

				156.97		99.73164

				156.99		99.73164

				157.01		99.73164

				157.04		99.72724

				157.06		99.72724

				157.08		99.72724

				157.1		99.72285

				157.12		99.71845

				157.14		99.71845

				157.16		99.71845

				157.18		99.71845

				157.2		99.71845

				157.23		99.71405

				157.25		99.71405

				157.27		99.71405

				157.29		99.71405

				157.31		99.70965

				157.33		99.70965

				157.35		99.70965

				157.37		99.70965

				157.39		99.70525

				157.42		99.70525

				157.44		99.70085

				157.46		99.70085

				157.48		99.70085

				157.5		99.69645

				157.52		99.69645

				157.54		99.69205

				157.56		99.69205

				157.59		99.68765

				157.61		99.68765

				157.63		99.68765

				157.65		99.68325

				157.67		99.68325

				157.69		99.67885

				157.71		99.67885

				157.73		99.67885

				157.75		99.67445

				157.78		99.67445

				157.8		99.67005

				157.82		99.67005

				157.84		99.66565

				157.86		99.66126

				157.88		99.66126

				157.9		99.65686

				157.92		99.65686

				157.94		99.65246

				157.97		99.65246

				157.99		99.64806

				158.01		99.64806

				158.03		99.64806

				158.05		99.64366

				158.07		99.64366

				158.09		99.64366

				158.11		99.63926

				158.14		99.63926

				158.16		99.63486

				158.18		99.63046

				158.2		99.63046

				158.22		99.63046

				158.24		99.62606

				158.26		99.62606

				158.28		99.62166

				158.3		99.61726

				158.33		99.61726

				158.35		99.61286

				158.37		99.61286

				158.39		99.61286

				158.41		99.60846

				158.43		99.60846

				158.45		99.60406

				158.47		99.59967

				158.49		99.59967

				158.52		99.59527

				158.54		99.59087

				158.56		99.59087

				158.58		99.59087

				158.6		99.58647

				158.62		99.58647

				158.64		99.58207

				158.66		99.57767

				158.68		99.57767

				158.71		99.57767

				158.73		99.57327

				158.75		99.57327

				158.77		99.56887

				158.79		99.56447

				158.81		99.56447

				158.83		99.56447

				158.85		99.56447

				158.88		99.56007

				158.9		99.56007

				158.92		99.55567

				158.94		99.55567

				158.96		99.55567

				158.98		99.55127

				159		99.55127

				159.02		99.55127

				159.04		99.55127

				159.07		99.54687

				159.09		99.54248

				159.11		99.54248

				159.13		99.53808

				159.15		99.53808

				159.17		99.53368

				159.19		99.53368

				159.21		99.53368

				159.23		99.52928

				159.26		99.52488

				159.28		99.52928

				159.3		99.52488

				159.32		99.52488

				159.34		99.52048

				159.36		99.51608

				159.38		99.51608

				159.4		99.51168

				159.42		99.51168

				159.45		99.51168

				159.47		99.50728

				159.49		99.50728

				159.51		99.50288

				159.53		99.50288

				159.55		99.49848

				159.57		99.49408

				159.59		99.49408

				159.61		99.49408

				159.64		99.48968

				159.66		99.48968

				159.68		99.48528

				159.7		99.48528

				159.72		99.48089

				159.74		99.47649

				159.76		99.47209

				159.78		99.47209

				159.8		99.46769

				159.83		99.46329

				159.85		99.46329

				159.87		99.46329

				159.89		99.46329

				159.91		99.45889

				159.93		99.45449

				159.95		99.45449

				159.97		99.45449

				160		99.45009

				160.02		99.45009

				160.04		99.45009

				160.06		99.44569

				160.08		99.44569

				160.1		99.44569

				160.12		99.44129

				160.14		99.44129

				160.16		99.44129

				160.19		99.44129

				160.21		99.43689

				160.23		99.43689

				160.25		99.43249

				160.27		99.43689

				160.29		99.43249

				160.31		99.43249

				160.33		99.42809

				160.35		99.42809

				160.38		99.42369

				160.4		99.4193

				160.42		99.4193

				160.44		99.4193

				160.46		99.4149

				160.48		99.4149

				160.5		99.4149

				160.52		99.4105

				160.54		99.4061

				160.57		99.4061

				160.59		99.4017

				160.61		99.3973

				160.63		99.3973

				160.65		99.3929

				160.67		99.3885

				160.69		99.3885

				160.71		99.3841

				160.73		99.3841

				160.76		99.3841

				160.78		99.3797

				160.8		99.3753

				160.82		99.3753

				160.84		99.3753

				160.86		99.3753

				160.88		99.3709

				160.9		99.3709

				160.92		99.3665

				160.95		99.3665

				160.97		99.3621

				160.99		99.35771

				161.01		99.35331

				161.03		99.35331

				161.05		99.35331

				161.07		99.34891

				161.09		99.34891

				161.11		99.34891

				161.14		99.34451

				161.16		99.34451

				161.18		99.34011

				161.2		99.34011

				161.22		99.33131

				161.24		99.33131

				161.26		99.33131

				161.28		99.32691

				161.3		99.32691

				161.33		99.32691

				161.35		99.32251

				161.37		99.31811

				161.39		99.31811

				161.41		99.31371

				161.43		99.31371

				161.45		99.31371

				161.47		99.30931

				161.49		99.30931

				161.52		99.30931

				161.54		99.30491

				161.56		99.30491

				161.58		99.30491

				161.6		99.30051

				161.62		99.30051

				161.64		99.29612

				161.66		99.29612

				161.68		99.29172

				161.71		99.29612

				161.73		99.29172

				161.75		99.28732

				161.77		99.28292

				161.79		99.28732

				161.81		99.27852

				161.83		99.27852

				161.85		99.27852

				161.87		99.27412

				161.9		99.26972

				161.92		99.26532

				161.94		99.26532

				161.96		99.26092

				161.98		99.26092

				162		99.25652

				162.02		99.25212

				162.04		99.25212

				162.06		99.24772

				162.09		99.24332

				162.11		99.24332

				162.13		99.23892

				162.15		99.23892

				162.17		99.23453

				162.19		99.23453

				162.21		99.23013

				162.23		99.22573

				162.25		99.22573

				162.28		99.22133

				162.3		99.22133

				162.32		99.22133

				162.34		99.21693

				162.36		99.21693

				162.38		99.21253

				162.4		99.21253

				162.42		99.20813

				162.44		99.20373

				162.47		99.20373

				162.49		99.20373

				162.51		99.19933

				162.53		99.19493

				162.55		99.19493

				162.57		99.19493

				162.59		99.19053

				162.61		99.18613

				162.63		99.18613

				162.66		99.18613

				162.68		99.18173

				162.7		99.17733

				162.72		99.17733

				162.74		99.17733

				162.76		99.17294

				162.78		99.16854

				162.8		99.16854

				162.82		99.16854

				162.85		99.16414

				162.87		99.16414

				162.89		99.15974

				162.91		99.15534

				162.93		99.15094

				162.95		99.15094

				162.97		99.15094

				162.99		99.14654

				163.01		99.14214

				163.03		99.14214

				163.06		99.14214

				163.08		99.13774

				163.1		99.13334

				163.12		99.13334

				163.14		99.12894

				163.16		99.12454

				163.18		99.12454

				163.2		99.12014

				163.22		99.11575

				163.25		99.11575

				163.27		99.10695

				163.29		99.11135

				163.31		99.10695

				163.33		99.10255

				163.35		99.10255

				163.37		99.09815

				163.39		99.09375

				163.41		99.09375

				163.44		99.08935

				163.46		99.08495

				163.48		99.08055

				163.5		99.07615

				163.52		99.07615

				163.54		99.07175

				163.56		99.06735

				163.58		99.06735

				163.6		99.06735

				163.62		99.06295

				163.65		99.05855

				163.67		99.05855

				163.69		99.05416

				163.71		99.05416

				163.73		99.05416

				163.75		99.04976

				163.77		99.04976

				163.79		99.04536

				163.81		99.04536

				163.84		99.04536

				163.86		99.04096

				163.88		99.03656

				163.9		99.03656

				163.92		99.03656

				163.94		99.03656

				163.96		99.03216

				163.98		99.02776

				164		99.02776

				164.03		99.02776

				164.05		99.01896

				164.07		99.01896

				164.09		99.01456

				164.11		99.01016

				164.13		99.01016

				164.15		99.00576

				164.17		99.00136

				164.19		99.00136

				164.21		98.99257

				164.24		98.99257

				164.26		98.99257

				164.28		98.98817

				164.3		98.98377

				164.32		98.98377

				164.34		98.98377

				164.36		98.97937

				164.38		98.97497

				164.4		98.97057

				164.43		98.97057

				164.45		98.96617

				164.47		98.96177

				164.49		98.96177

				164.51		98.96177

				164.53		98.95737

				164.55		98.95737

				164.57		98.95737

				164.59		98.95297

				164.62		98.95297

				164.64		98.94857

				164.66		98.94857

				164.68		98.94417

				164.7		98.94417

				164.72		98.93977

				164.74		98.93537

				164.76		98.93537

				164.78		98.93098

				164.8		98.93098

				164.83		98.93098

				164.85		98.92658

				164.87		98.92658

				164.89		98.92218

				164.91		98.91778

				164.93		98.91778

				164.95		98.91338

				164.97		98.91338

				164.99		98.90898

				165.02		98.90458

				165.04		98.90458

				165.06		98.90018

				165.08		98.90018

				165.1		98.89578

				165.12		98.89138

				165.14		98.89138

				165.16		98.89138

				165.18		98.88698

				165.2		98.88698

				165.23		98.88258

				165.25		98.88258

				165.27		98.87818

				165.29		98.87378

				165.31		98.87378

				165.33		98.86939

				165.35		98.86499

				165.37		98.86059

				165.39		98.86059

				165.42		98.85619

				165.44		98.85619

				165.46		98.85179

				165.48		98.85179

				165.5		98.84739

				165.52		98.84299

				165.54		98.84299

				165.56		98.83859

				165.58		98.83859

				165.6		98.83419

				165.63		98.82979

				165.65		98.82539

				165.67		98.82099

				165.69		98.81659

				165.71		98.81659

				165.73		98.81219

				165.75		98.81219

				165.77		98.8078

				165.79		98.8034

				165.82		98.799

				165.84		98.7946

				165.86		98.7902

				165.88		98.7902

				165.9		98.7858

				165.92		98.7814

				165.94		98.777

				165.96		98.7726

				165.98		98.7726

				166		98.7682

				166.03		98.7638

				166.05		98.7638

				166.07		98.7638

				166.09		98.7638

				166.11		98.7594

				166.13		98.755

				166.15		98.7506

				166.17		98.7506

				166.19		98.7506

				166.22		98.7506

				166.24		98.74621

				166.26		98.74621

				166.28		98.74181

				166.3		98.74181

				166.32		98.73741

				166.34		98.73301

				166.36		98.72861

				166.38		98.72861

				166.4		98.72421

				166.43		98.71981

				166.45		98.71541

				166.47		98.70661

				166.49		98.70221

				166.51		98.70221

				166.53		98.70221

				166.55		98.69781

				166.57		98.68902

				166.59		98.68902

				166.62		98.68902

				166.64		98.68462

				166.66		98.68462

				166.68		98.68022

				166.7		98.67582

				166.72		98.67142

				166.74		98.67142

				166.76		98.66702

				166.78		98.66702

				166.8		98.66262

				166.83		98.66262

				166.85		98.66262

				166.87		98.66262

				166.89		98.65822

				166.91		98.65382

				166.93		98.65382

				166.95		98.64942

				166.97		98.64942

				166.99		98.64502

				167.01		98.64502

				167.04		98.64062

				167.06		98.64062

				167.08		98.63182

				167.1		98.63622

				167.12		98.63182

				167.14		98.62743

				167.16		98.62303

				167.18		98.62303

				167.2		98.61863

				167.23		98.61863

				167.25		98.60983

				167.27		98.60983

				167.29		98.60103

				167.31		98.60103

				167.33		98.59223

				167.35		98.59223

				167.37		98.58783

				167.39		98.58343

				167.42		98.57903

				167.44		98.57903

				167.46		98.57023

				167.48		98.56584

				167.5		98.56584

				167.52		98.56584

				167.54		98.56144

				167.56		98.55704

				167.58		98.55704

				167.6		98.55704

				167.63		98.55264

				167.65		98.55264

				167.67		98.54824

				167.69		98.54824

				167.71		98.54384

				167.73		98.54384

				167.75		98.53504

				167.77		98.53504

				167.79		98.53064

				167.81		98.52624

				167.84		98.52184

				167.86		98.51744

				167.88		98.51304

				167.9		98.50864

				167.92		98.50425

				167.94		98.49985

				167.96		98.49545

				167.98		98.49545

				168		98.49105

				168.03		98.49105

				168.05		98.48665

				168.07		98.48225

				168.09		98.48225

				168.11		98.47785

				168.13		98.47785

				168.15		98.47345

				168.17		98.46905

				168.19		98.47345

				168.21		98.46905

				168.24		98.46465

				168.26		98.46905

				168.28		98.46465

				168.3		98.46025

				168.32		98.45585

				168.34		98.45145

				168.36		98.45145

				168.38		98.44705

				168.4		98.44266

				168.43		98.44266

				168.45		98.43826

				168.47		98.43826

				168.49		98.43386

				168.51		98.42946

				168.53		98.42506

				168.55		98.42506

				168.57		98.42066

				168.59		98.42066

				168.62		98.41186

				168.64		98.41186

				168.66		98.40746

				168.68		98.40746

				168.7		98.40746

				168.72		98.40746

				168.74		98.40306

				168.76		98.39866

				168.78		98.39426

				168.8		98.39426

				168.83		98.38986

				168.85		98.38546

				168.87		98.38546

				168.89		98.38107

				168.91		98.37667

				168.93		98.37227

				168.95		98.37227

				168.97		98.36787

				168.99		98.36787

				169.02		98.36347

				169.04		98.35907

				169.06		98.35027

				169.08		98.35027

				169.1		98.34587

				169.12		98.34587

				169.14		98.33707

				169.16		98.33267

				169.18		98.33267

				169.2		98.32827

				169.23		98.31948

				169.25		98.31948

				169.27		98.31508

				169.29		98.31068

				169.31		98.30628

				169.33		98.30188

				169.35		98.29748

				169.37		98.29748

				169.39		98.29308

				169.42		98.28868

				169.44		98.29308

				169.46		98.28428

				169.48		98.27988

				169.5		98.27548

				169.52		98.27548

				169.54		98.27108

				169.56		98.26668

				169.58		98.26228

				169.6		98.26228

				169.63		98.25789

				169.65		98.24909

				169.67		98.24469

				169.69		98.24469

				169.71		98.23589

				169.73		98.23149

				169.75		98.22709

				169.77		98.22269

				169.79		98.21829

				169.81		98.21389

				169.84		98.20949

				169.86		98.20509

				169.88		98.1963

				169.9		98.1919

				169.92		98.1963

				169.94		98.1875

				169.96		98.1831

				169.98		98.1831

				170		98.1787

				170.03		98.1743

				170.05		98.1699

				170.07		98.1699

				170.09		98.1611

				170.11		98.1611

				170.13		98.1567

				170.15		98.1567

				170.17		98.1523

				170.19		98.1523

				170.21		98.1479

				170.24		98.13911

				170.26		98.13911

				170.28		98.13471

				170.3		98.13031

				170.32		98.13031

				170.34		98.12591

				170.36		98.12591

				170.38		98.12151

				170.4		98.11711

				170.42		98.11271

				170.45		98.10831

				170.47		98.10831

				170.49		98.09951

				170.51		98.09951

				170.53		98.09511

				170.55		98.09511

				170.57		98.09071

				170.59		98.08631

				170.61		98.08631

				170.64		98.08191

				170.66		98.07752

				170.68		98.07312

				170.7		98.06872

				170.72		98.06432

				170.74		98.05992

				170.76		98.05552

				170.78		98.05112

				170.8		98.04672

				170.82		98.04232

				170.85		98.03792

				170.87		98.03792

				170.89		98.03352

				170.91		98.03352

				170.93		98.02472

				170.95		98.02472

				170.97		98.02032

				170.99		98.02032

				171.01		98.01153

				171.03		98.00713

				171.06		98.00273

				171.08		98.00273

				171.1		97.99393

				171.12		97.98953

				171.14		97.98513

				171.16		97.98513

				171.18		97.97633

				171.2		97.97633

				171.22		97.97193

				171.24		97.96753

				171.27		97.96313

				171.29		97.96753

				171.31		97.96313

				171.33		97.96313

				171.35		97.95434

				171.37		97.95434

				171.39		97.94554

				171.41		97.94554

				171.43		97.94114

				171.45		97.93234

				171.48		97.93234

				171.5		97.92794

				171.52		97.91914

				171.54		97.91474

				171.56		97.90594

				171.58		97.90154

				171.6		97.89714

				171.62		97.89275

				171.64		97.88835

				171.66		97.88395

				171.69		97.87955

				171.71		97.87515

				171.73		97.87515

				171.75		97.86635

				171.77		97.86195

				171.79		97.86195

				171.81		97.85755

				171.83		97.85755

				171.85		97.85755

				171.87		97.85755

				171.9		97.85315

				171.92		97.84875

				171.94		97.84435

				171.96		97.84435

				171.98		97.83555

				172		97.83116

				172.02		97.83116

				172.04		97.83116

				172.06		97.82676

				172.09		97.82236

				172.11		97.81356

				172.13		97.80916

				172.15		97.80036

				172.17		97.79596

				172.19		97.79156

				172.21		97.79156

				172.23		97.78276

				172.25		97.77836

				172.27		97.77836

				172.3		97.76957

				172.32		97.76517

				172.34		97.76517

				172.36		97.75637

				172.38		97.75637

				172.4		97.75637

				172.42		97.75197

				172.44		97.75197

				172.46		97.74757

				172.48		97.74317

				172.51		97.73877

				172.53		97.73877

				172.55		97.72997

				172.57		97.72557

				172.59		97.72557

				172.61		97.71677

				172.63		97.71677

				172.65		97.71238

				172.67		97.70798

				172.69		97.70358

				172.72		97.69478

				172.74		97.69038

				172.76		97.69038

				172.78		97.68158

				172.8		97.67718

				172.82		97.67718

				172.84		97.67278

				172.86		97.66838

				172.88		97.66398

				172.9		97.65958

				172.93		97.65958

				172.95		97.65518

				172.97		97.65079

				172.99		97.64639

				173.01		97.64199

				173.03		97.63759

				173.05		97.63319

				173.07		97.62879

				173.09		97.62879

				173.12		97.62439

				173.14		97.61999

				173.16		97.61559

				173.18		97.61559

				173.2		97.60679

				173.22		97.60679

				173.24		97.60239

				173.26		97.59799

				173.28		97.59359

				173.3		97.5892

				173.33		97.5848

				173.35		97.5804

				173.37		97.5716

				173.39		97.5716

				173.41		97.5672

				173.43		97.5584

				173.45		97.5496

				173.47		97.5452

				173.49		97.5408

				173.51		97.5408

				173.54		97.532

				173.56		97.532

				173.58		97.52321

				173.6		97.51881

				173.62		97.51441

				173.64		97.51001

				173.66		97.50561

				173.68		97.50561

				173.7		97.49681

				173.72		97.49241

				173.75		97.48361

				173.77		97.48361

				173.79		97.47481

				173.81		97.47041

				173.83		97.46602

				173.85		97.46602

				173.87		97.46602

				173.89		97.46162

				173.91		97.46162

				173.93		97.45722

				173.95		97.44842

				173.98		97.44842

				174		97.44402

				174.02		97.43962

				174.04		97.43962

				174.06		97.43082

				174.08		97.42642

				174.1		97.41762

				174.12		97.40882

				174.14		97.40882

				174.16		97.40443

				174.19		97.40003

				174.21		97.39563

				174.23		97.38683

				174.25		97.38243

				174.27		97.37803

				174.29		97.37363

				174.31		97.37363

				174.33		97.36483

				174.35		97.36483

				174.37		97.35603

				174.4		97.35603

				174.42		97.35163

				174.44		97.34724

				174.46		97.34284

				174.48		97.33844

				174.5		97.32964

				174.52		97.32964

				174.54		97.32084

				174.56		97.32084

				174.59		97.30764

				174.61		97.30764

				174.63		97.29884

				174.65		97.29444

				174.67		97.28565

				174.69		97.28125

				174.71		97.27685

				174.73		97.27245

				174.75		97.26805

				174.77		97.26365

				174.8		97.25485

				174.82		97.25045

				174.84		97.25045

				174.86		97.24165

				174.88		97.24605

				174.9		97.24165

				174.92		97.23725

				174.94		97.23725

				174.96		97.23285

				174.98		97.22406

				175.01		97.22406

				175.03		97.21526

				175.05		97.21526

				175.07		97.20646

				175.09		97.20206

				175.11		97.19326

				175.13		97.18446

				175.15		97.18006

				175.17		97.17126

				175.19		97.17126

				175.22		97.16686

				175.24		97.16247

				175.26		97.15807

				175.28		97.15367

				175.3		97.14927

				175.32		97.14927

				175.34		97.14487

				175.36		97.14487

				175.38		97.14047

				175.4		97.13607

				175.43		97.13167

				175.45		97.12727

				175.47		97.12287

				175.49		97.11847

				175.51		97.11407

				175.53		97.10967

				175.55		97.10527

				175.57		97.10088

				175.59		97.09208

				175.61		97.09208

				175.64		97.08328

				175.66		97.07888

				175.68		97.07448

				175.7		97.07008

				175.72		97.06128

				175.74		97.05688

				175.76		97.05248

				175.78		97.04808

				175.8		97.03929

				175.82		97.03929

				175.85		97.03489

				175.87		97.03049

				175.89		97.02609

				175.91		97.02169

				175.93		97.01289

				175.95		97.01289

				175.97		97.00409

				175.99		97.00409

				176.01		96.99089

				176.03		96.98649

				176.06		96.98209

				176.08		96.9777

				176.1		96.9689

				176.12		96.9645

				176.14		96.9601

				176.16		96.9601

				176.18		96.9513

				176.2		96.9513

				176.22		96.9469

				176.24		96.9469

				176.26		96.9337

				176.29		96.9293

				176.31		96.92051

				176.33		96.91611

				176.35		96.90731

				176.37		96.90291

				176.39		96.89851

				176.41		96.89411

				176.43		96.88971

				176.45		96.88091

				176.47		96.87211

				176.5		96.87211

				176.52		96.86771

				176.54		96.86771

				176.56		96.85452

				176.58		96.85012

				176.6		96.84132

				176.62		96.83692

				176.64		96.83252

				176.66		96.82812

				176.68		96.81932

				176.71		96.81492

				176.73		96.80612

				176.75		96.80172

				176.77		96.79733

				176.79		96.79293

				176.81		96.78413

				176.83		96.78413

				176.85		96.77533

				176.87		96.77533

				176.89		96.76653

				176.92		96.76653

				176.94		96.76213

				176.96		96.75773

				176.98		96.75773

				177		96.74893

				177.02		96.74453

				177.04		96.74453

				177.06		96.73574

				177.08		96.73574

				177.1		96.73134

				177.13		96.73134

				177.15		96.72254

				177.17		96.71814

				177.19		96.70934

				177.21		96.70494

				177.23		96.70054

				177.25		96.69614

				177.27		96.68734

				177.29		96.68294

				177.31		96.67415

				177.33		96.66975

				177.36		96.66535

				177.38		96.66095

				177.4		96.66095

				177.42		96.65655

				177.44		96.65215

				177.46		96.65215

				177.48		96.64335

				177.5		96.63895

				177.52		96.63455

				177.54		96.63015

				177.57		96.62135

				177.59		96.61256

				177.61		96.60816

				177.63		96.59936

				177.65		96.59056

				177.67		96.59056

				177.69		96.58176

				177.71		96.57736

				177.73		96.57296

				177.75		96.57296

				177.77		96.56416

				177.8		96.55976

				177.82		96.55976

				177.84		96.55097

				177.86		96.54657

				177.88		96.54217

				177.9		96.53777

				177.92		96.53337

				177.94		96.52457

				177.96		96.52017

				177.98		96.51577

				178.01		96.51577

				178.03		96.50257

				178.05		96.50257

				178.07		96.49817

				178.09		96.49378

				178.11		96.48938

				178.13		96.48498

				178.15		96.47618

				178.17		96.46738

				178.19		96.45858

				178.21		96.44978

				178.24		96.44538

				178.26		96.44098

				178.28		96.44538

				178.3		96.43658

				178.32		96.43219

				178.34		96.42779

				178.36		96.42339

				178.38		96.41459

				178.4		96.41459

				178.42		96.41019

				178.45		96.39699

				178.47		96.38819

				178.49		96.37939

				178.51		96.37499

				178.53		96.3706

				178.55		96.3618

				178.57		96.3574

				178.59		96.3574

				178.61		96.3486

				178.63		96.3486

				178.66		96.3486

				178.68		96.3442

				178.7		96.3354

				178.72		96.331

				178.74		96.331

				178.76		96.3178

				178.78		96.30901

				178.8		96.30901

				178.82		96.30461

				178.84		96.29581

				178.86		96.29141

				178.89		96.29141

				178.91		96.28261

				178.93		96.27821

				178.95		96.28261

				178.97		96.27821

				178.99		96.26941

				179.01		96.25621

				179.03		96.24742

				179.05		96.24742

				179.07		96.23862

				179.1		96.23422

				179.12		96.22542

				179.14		96.22102

				179.16		96.21222

				179.18		96.20782

				179.2		96.20782

				179.22		96.20342

				179.24		96.19902

				179.26		96.19022

				179.28		96.18583

				179.3		96.17703

				179.33		96.17703

				179.35		96.16823

				179.37		96.16823

				179.39		96.15503

				179.41		96.15063

				179.43		96.14623

				179.45		96.13743

				179.47		96.13303

				179.49		96.13303

				179.51		96.12424

				179.54		96.11984

				179.56		96.11104

				179.58		96.11544

				179.6		96.10664

				179.62		96.10224

				179.64		96.10224

				179.66		96.09344

				179.68		96.08904

				179.7		96.08464

				179.72		96.08464

				179.74		96.08024

				179.77		96.06265

				179.79		96.06265

				179.81		96.05385

				179.83		96.04945

				179.85		96.04505

				179.87		96.04505

				179.89		96.03185

				179.91		96.02745

				179.93		96.01425

				179.95		96.01865

				179.98		96.00546

				180		95.99666

				180.02		95.99226

				180.04		95.98786

				180.06		95.97466

				180.08		95.97466

				180.1		95.96586

				180.12		95.96146

				180.14		95.94826

				180.16		95.94387

				180.19		95.93507

				180.21		95.93507

				180.23		95.92187

				180.25		95.91747

				180.27		95.90867

				180.29		95.89987

				180.31		95.89987

				180.33		95.89547

				180.35		95.88667

				180.37		95.88667

				180.4		95.87788

				180.42		95.87348

				180.44		95.87348

				180.46		95.86908

				180.48		95.86468

				180.5		95.85588

				180.52		95.85148

				180.54		95.84708

				180.56		95.84268

				180.58		95.83388

				180.61		95.82508

				180.63		95.81629

				180.65		95.81189

				180.67		95.80749

				180.69		95.80309

				180.71		95.79429

				180.73		95.78989

				180.75		95.78109

				180.77		95.77669

				180.79		95.77229

				180.81		95.7591

				180.84		95.7547

				180.86		95.7503

				180.88		95.7415

				180.9		95.7371

				180.92		95.7283

				180.94		95.7239

				180.96		95.7107

				180.98		95.7019

				181		95.7019

				181.02		95.68871

				181.05		95.68431

				181.07		95.67551

				181.09		95.67111

				181.11		95.66671

				181.13		95.66231

				181.15		95.66671

				181.17		95.66231

				181.19		95.65351

				181.21		95.65351

				181.23		95.64911

				181.26		95.64911

				181.28		95.64471

				181.3		95.63592

				181.32		95.62712

				181.34		95.61392

				181.36		95.60952

				181.38		95.60512

				181.4		95.60952

				181.42		95.60072

				181.44		95.59192

				181.46		95.58752

				181.49		95.57433

				181.51		95.56993

				181.53		95.56553

				181.55		95.55673

				181.57		95.54793

				181.59		95.53033

				181.61		95.52593

				181.63		95.52593

				181.65		95.51274

				181.67		95.50834

				181.7		95.50834

				181.72		95.49954

				181.74		95.49514

				181.76		95.48634

				181.78		95.48634

				181.8		95.47314

				181.82		95.46874

				181.84		95.45994

				181.86		95.45555

				181.88		95.44675

				181.91		95.44235

				181.93		95.43795

				181.95		95.43795

				181.97		95.42035

				181.99		95.42035

				182.01		95.41155

				182.03		95.40715

				182.05		95.39835

				182.07		95.38956

				182.09		95.38516

				182.11		95.37636

				182.14		95.36756

				182.16		95.36756

				182.18		95.35876

				182.2		95.35436

				182.22		95.34996

				182.24		95.34556

				182.26		95.34116

				182.28		95.34116

				182.3		95.32357

				182.32		95.31477

				182.35		95.30597

				182.37		95.29717

				182.39		95.28837

				182.41		95.27957

				182.43		95.27957

				182.45		95.27957

				182.47		95.27517

				182.49		95.26198

				182.51		95.25758

				182.53		95.25318

				182.56		95.24438

				182.58		95.23118

				182.6		95.22678

				182.62		95.21358

				182.64		95.21358

				182.66		95.20919

				182.68		95.21358

				182.7		95.20479

				182.72		95.20479

				182.74		95.19159

				182.76		95.19159

				182.79		95.18279

				182.81		95.18279

				182.83		95.16519

				182.85		95.16079

				182.87		95.152

				182.89		95.1432

				182.91		95.13

				182.93		95.1256

				182.95		95.1168

				182.97		95.1168

				183		95.108

				183.02		95.1036

				183.04		95.0992

				183.06		95.09041

				183.08		95.07721

				183.1		95.06841

				183.12		95.05961

				183.14		95.05081

				183.16		95.04641

				183.18		95.03321

				183.2		95.02882

				183.23		95.02442

				183.25		95.01122

				183.27		95.01122

				183.29		95.00682

				183.31		95.00242

				183.33		94.99802

				183.35		94.98922

				183.37		94.98922

				183.39		94.98922

				183.41		94.97162

				183.44		94.96723

				183.46		94.94963

				183.48		94.94963

				183.5		94.93643

				183.52		94.93203

				183.54		94.92323

				183.56		94.91883

				183.58		94.91003

				183.6		94.91003

				183.62		94.90564

				183.64		94.91003

				183.67		94.89244

				183.69		94.88804

				183.71		94.88364

				183.73		94.87924

				183.75		94.87484

				183.77		94.86604

				183.79		94.85284

				183.81		94.85284

				183.83		94.84844

				183.85		94.83965

				183.88		94.83085

				183.9		94.82645

				183.92		94.81325

				183.94		94.80445

				183.96		94.80005

				183.98		94.78685

				184		94.77366

				184.02		94.76486

				184.04		94.75166

				184.06		94.75606

				184.08		94.74286

				184.11		94.73846

				184.13		94.72966

				184.15		94.72966

				184.17		94.72087

				184.19		94.71647

				184.21		94.70327

				184.23		94.70327

				184.25		94.69887

				184.27		94.69007

				184.29		94.68127

				184.32		94.67687

				184.34		94.66807

				184.36		94.66368

				184.38		94.65048

				184.4		94.64608

				184.42		94.64168

				184.44		94.63728

				184.46		94.62848

				184.48		94.62408

				184.5		94.61528

				184.52		94.61088

				184.55		94.60209

				184.57		94.58449

				184.59		94.58009

				184.61		94.57129

				184.63		94.54929

				184.65		94.5405

				184.67		94.5273

				184.69		94.5185

				184.71		94.5185

				184.73		94.5141

				184.75		94.5053

				184.78		94.5141

				184.8		94.5053

				184.82		94.4965

				184.84		94.4921

				184.86		94.47891

				184.88		94.47011

				184.9		94.47011

				184.92		94.45691

				184.94		94.45691

				184.96		94.45691

				184.99		94.44371

				185.01		94.44811

				185.03		94.43931

				185.05		94.43051

				185.07		94.42171

				185.09		94.41732

				185.11		94.40412

				185.13		94.39972

				185.15		94.39092

				185.17		94.38212

				185.19		94.37772

				185.22		94.37332

				185.24		94.36012

				185.26		94.36012

				185.28		94.35133

				185.3		94.34693

				185.32		94.34253

				185.34		94.33373

				185.36		94.32493

				185.38		94.32053

				185.4		94.31173

				185.42		94.30733

				185.45		94.29854

				185.47		94.28974

				185.49		94.28094

				185.51		94.27214

				185.53		94.26334

				185.55		94.25014

				185.57		94.24134

				185.59		94.23255

				185.61		94.22815

				185.63		94.21495

				185.65		94.21495

				185.68		94.21055

				185.7		94.20615

				185.72		94.19295

				185.74		94.19295

				185.76		94.18415

				185.78		94.17536

				185.8		94.16656

				185.82		94.15776

				185.84		94.14456

				185.86		94.14456

				185.89		94.12696

				185.91		94.11816

				185.93		94.10937

				185.95		94.10057

				185.97		94.10057

				185.99		94.09177

				186.01		94.08737

				186.03		94.08297

				186.05		94.07417

				186.07		94.06537

				186.09		94.05657

				186.12		94.04338

				186.14		94.03458

				186.16		94.02578

				186.18		94.01698

				186.2		94.01698

				186.22		94.02138

				186.24		93.99938

				186.26		93.99938

				186.28		93.99498

				186.3		93.98619

				186.33		93.96859

				186.35		93.96419

				186.37		93.94659

				186.39		93.94219

				186.41		93.93339

				186.43		93.929

				186.45		93.929

				186.47		93.9246

				186.49		93.9158

				186.51		93.9158

				186.53		93.9158

				186.56		93.907

				186.58		93.8982

				186.6		93.8894

				186.62		93.8806

				186.64		93.8762

				186.66		93.86301

				186.68		93.85421

				186.7		93.84541

				186.72		93.83221

				186.74		93.82341

				186.76		93.81901

				186.79		93.81022

				186.81		93.80582

				186.83		93.78822

				186.85		93.78822

				186.87		93.77942

				186.89		93.77502

				186.91		93.76622

				186.93		93.76182

				186.95		93.74423

				186.97		93.73983

				187		93.73103

				187.02		93.72663

				187.04		93.71343

				187.06		93.70463

				187.08		93.68704

				187.1		93.68704

				187.12		93.67384

				187.14		93.66064

				187.16		93.65184

				187.18		93.64304

				187.2		93.63864

				187.23		93.62984

				187.25		93.61225

				187.27		93.60785

				187.29		93.59465

				187.31		93.59025

				187.33		93.58145

				187.35		93.57265

				187.37		93.55946

				187.39		93.55506

				187.41		93.54626

				187.43		93.54626

				187.46		93.52866

				187.48		93.52866

				187.5		93.51546

				187.52		93.51106

				187.54		93.50227

				187.56		93.49347

				187.58		93.48027

				187.6		93.48027

				187.62		93.46707

				187.64		93.46267

				187.66		93.44947

				187.69		93.44508

				187.71		93.43628

				187.73		93.43188

				187.75		93.41428

				187.77		93.40988

				187.79		93.40108

				187.81		93.39228

				187.83		93.38349

				187.85		93.36589

				187.87		93.35709

				187.9		93.35269

				187.92		93.33949

				187.94		93.33069

				187.96		93.32629

				187.98		93.3131

				188		93.3131

				188.02		93.3087

				188.04		93.3043

				188.06		93.2955

				188.08		93.2911

				188.1		93.2823

				188.13		93.2779

				188.15		93.2691

				188.17		93.25591

				188.19		93.24271

				188.21		93.23391

				188.23		93.22071

				188.25		93.21631

				188.27		93.20311

				188.29		93.18992

				188.31		93.18552

				188.33		93.17672

				188.36		93.16792

				188.38		93.16352

				188.4		93.15472

				188.42		93.15032

				188.44		93.15032

				188.46		93.14152

				188.48		93.13713

				188.5		93.12393

				188.52		93.11953

				188.54		93.10633

				188.57		93.10193

				188.59		93.09313

				188.61		93.07114

				188.63		93.07993

				188.65		93.06674

				188.67		93.06674

				188.69		93.04914

				188.71		93.04474

				188.73		93.02274

				188.75		93.01834

				188.77		93.00515

				188.8		93.00075

				188.82		92.99635

				188.84		92.99195

				188.86		92.96995

				188.88		92.95676

				188.9		92.94356

				188.92		92.93476

				188.94		92.92156

				188.96		92.91716

				188.98		92.90836

				189		92.90836

				189.03		92.89077

				189.05		92.88637

				189.07		92.87317

				189.09		92.86437

				189.11		92.84677

				189.13		92.84677

				189.15		92.83797

				189.17		92.84237

				189.19		92.82478

				189.21		92.82038

				189.23		92.80278

				189.26		92.79838

				189.28		92.78078

				189.3		92.78518

				189.32		92.77199

				189.34		92.77199

				189.36		92.74559

				189.38		92.73239

				189.4		92.71919

				189.42		92.71479

				189.44		92.6972

				189.47		92.706

				189.49		92.6972

				189.51		92.6928

				189.53		92.6796

				189.55		92.6752

				189.57		92.6664

				189.59		92.6532

				189.61		92.64001

				189.63		92.62681

				189.65		92.61801

				189.67		92.60481

				189.7		92.60481

				189.72		92.60041

				189.74		92.60041

				189.76		92.59161

				189.78		92.58282

				189.8		92.56962

				189.82		92.56082

				189.84		92.54762

				189.86		92.53442

				189.88		92.53003

				189.9		92.52123

				189.93		92.50803

				189.95		92.50363

				189.97		92.49923

				189.99		92.49043

				190.01		92.49043

				190.03		92.48163

				190.05		92.47723

				190.07		92.46404

				190.09		92.45964

				190.11		92.44644

				190.13		92.43764

				190.16		92.42444

				190.18		92.41564

				190.2		92.39365

				190.22		92.38925

				190.24		92.37605

				190.26		92.37165

				190.28		92.36725

				190.3		92.37165

				190.32		92.36285

				190.34		92.34965

				190.37		92.34086

				190.39		92.33206

				190.41		92.32326

				190.43		92.31446

				190.45		92.31006

				190.47		92.29246

				190.49		92.28367

				190.51		92.26607

				190.53		92.25287

				190.55		92.23967

				190.57		92.23087

				190.6		92.22208

				190.62		92.21328

				190.64		92.20008

				190.66		92.20008

				190.68		92.20008

				190.7		92.19568

				190.72		92.18688

				190.74		92.18248

				190.76		92.16928

				190.78		92.15609

				190.8		92.14289

				190.83		92.13409

				190.85		92.12089

				190.87		92.11649

				190.89		92.11209

				190.91		92.0989

				190.93		92.0901

				190.95		92.0769

				190.97		92.0681

				190.99		92.0549

				191.01		92.0549

				191.03		92.0505

				191.06		92.03731

				191.08		92.02411

				191.1		92.01531

				191.12		92.00651

				191.14		91.99771

				191.16		91.98891

				191.18		91.98451

				191.2		91.98451

				191.22		91.95812

				191.24		91.94932

				191.26		91.94492

				191.29		91.92292

				191.31		91.90533

				191.33		91.90973

				191.35		91.89213

				191.37		91.88333

				191.39		91.87013

				191.41		91.86133

				191.43		91.85694

				191.45		91.85254

				191.47		91.84374

				191.49		91.84814

				191.52		91.83494

				191.54		91.83054

				191.56		91.82174

				191.58		91.80414

				191.6		91.79095

				191.62		91.78215

				191.64		91.76455

				191.66		91.75135

				191.68		91.74255

				191.7		91.74255

				191.73		91.72496

				191.75		91.72056

				191.77		91.71616

				191.79		91.71176

				191.81		91.69416

				191.83		91.68976

				191.85		91.67657

				191.87		91.66777

				191.89		91.64577

				191.91		91.64137

				191.93		91.62817

				191.96		91.63257

				191.98		91.60618

				192		91.60178

				192.02		91.59298

				192.04		91.58858

				192.06		91.56218

				192.08		91.56218

				192.1		91.55778

				192.12		91.54019

				192.14		91.51819

				192.16		91.51379

				192.19		91.50499

				192.21		91.49619

				192.23		91.4874

				192.25		91.4786

				192.27		91.4698

				192.29		91.461

				192.31		91.4478

				192.33		91.439

				192.35		91.439

				192.37		91.42141

				192.39		91.40821

				192.42		91.40381

				192.44		91.39061

				192.46		91.37741

				192.48		91.37301

				192.5		91.37301

				192.52		91.35542

				192.54		91.35102

				192.56		91.33782

				192.58		91.32902

				192.6		91.31142

				192.62		91.30263

				192.65		91.28503

				192.67		91.27623

				192.69		91.26743

				192.71		91.25863

				192.73		91.24984

				192.75		91.24984

				192.77		91.22784

				192.79		91.21464

				192.81		91.20144

				192.83		91.19264

				192.86		91.17945

				192.88		91.17945

				192.9		91.17065

				192.92		91.16185

				192.94		91.15305

				192.96		91.14425

				192.98		91.13545

				193		91.12666

				193.02		91.11346

				193.04		91.10466

				193.06		91.08266

				193.09		91.07386

				193.11		91.06507

				193.13		91.05627

				193.15		91.04747

				193.17		91.04307

				193.19		91.03427

				193.21		91.01667

				193.23		91.00348

				193.25		90.99028

				193.27		90.97268

				193.29		90.96388

				193.32		90.94628

				193.34		90.94189

				193.36		90.94189

				193.38		90.92869

				193.4		90.93309

				193.42		90.93309

				193.44		90.91549

				193.46		90.90669

				193.48		90.90229

				193.5		90.88469

				193.52		90.8671

				193.55		90.8583

				193.57		90.8407

				193.59		90.8363

				193.61		90.81431

				193.63		90.80551

				193.65		90.80551

				193.67		90.79231

				193.69		90.77471

				193.71		90.77471

				193.73		90.76591

				193.75		90.75272

				193.78		90.74392

				193.8		90.73952

				193.82		90.73072

				193.84		90.72192

				193.86		90.69993

				193.88		90.69553

				193.9		90.68233

				193.92		90.66473

				193.94		90.65593

				193.96		90.65593

				193.98		90.63834

				194.01		90.62954

				194.03		90.61634

				194.05		90.61194

				194.07		90.59434

				194.09		90.58114

				194.11		90.55915

				194.13		90.56355

				194.15		90.53715

				194.17		90.53715

				194.19		90.52395

				194.22		90.53275

				194.24		90.51516

				194.26		90.51955

				194.28		90.49316

				194.3		90.49316

				194.32		90.46236

				194.34		90.44917

				194.36		90.43157

				194.38		90.43157

				194.4		90.41397

				194.42		90.41837

				194.45		90.40957

				194.47		90.40517

				194.49		90.39198

				194.51		90.37878

				194.53		90.35678

				194.55		90.34358

				194.57		90.33479

				194.59		90.32599

				194.61		90.31719

				194.63		90.31279

				194.65		90.29519

				194.68		90.2732

				194.7		90.26

				194.72		90.2556

				194.74		90.238

				194.76		90.2424

				194.78		90.2424

				194.8		90.2292

				194.82		90.2204

				194.84		90.2204

				194.86		90.19401

				194.88		90.18961

				194.91		90.18081

				194.93		90.15881

				194.95		90.13242

				194.97		90.13682

				194.99		90.10602

				195.01		90.09722

				195.03		90.08403

				195.05		90.08403

				195.07		90.07083

				195.09		90.06643

				195.11		90.04443

				195.14		90.04443

				195.16		90.02684

				195.18		90.01364

				195.2		90.00044

				195.22		90.00044

				195.24		89.97844

				195.26		89.97844

				195.28		89.96525

				195.3		89.95645

				195.32		89.94765

				195.34		89.93885

				195.37		89.92125

				195.39		89.91245

				195.41		89.90806

				195.43		89.89486

				195.45		89.88166

				195.47		89.87286

				195.49		89.85526

				195.51		89.84207

				195.53		89.83327

				195.55		89.81567

				195.58		89.80687

				195.6		89.79807

				195.62		89.78488

				195.64		89.77608

				195.66		89.76728

				195.68		89.75848

				195.7		89.74088

				195.72		89.73208

				195.74		89.71449

				195.76		89.70569

				195.78		89.69249

				195.81		89.68809

				195.83		89.67049

				195.85		89.66609

				195.87		89.6573

				195.89		89.6441

				195.91		89.6397

				195.93		89.6309

				195.95		89.6133

				195.97		89.6133

				195.99		89.59131

				196.01		89.56931

				196.04		89.56051

				196.06		89.54731

				196.08		89.52972

				196.1		89.52972

				196.12		89.52532

				196.14		89.51652

				196.16		89.50772

				196.18		89.49452

				196.2		89.48133

				196.22		89.46813

				196.25		89.45493

				196.27		89.44613

				196.29		89.42853

				196.31		89.41974

				196.33		89.41094

				196.35		89.40214

				196.37		89.38014

				196.39		89.37574

				196.41		89.35815

				196.43		89.34055

				196.45		89.32735

				196.48		89.33175

				196.5		89.32295

				196.52		89.31855

				196.54		89.29656

				196.56		89.28336

				196.58		89.26136

				196.6		89.24376

				196.62		89.23057

				196.64		89.23057

				196.66		89.21297

				196.68		89.20417

				196.71		89.18657

				196.73		89.17777

				196.75		89.16018

				196.77		89.15138

				196.79		89.13378

				196.81		89.12938

				196.83		89.11179

				196.85		89.10299

				196.87		89.09859

				196.89		89.08979

				196.91		89.08099

				196.94		89.07219

				196.96		89.05899

				196.98		89.0414

				197		89.0326

				197.02		89.015

				197.04		89.0018

				197.06		88.9974

				197.08		88.98421

				197.1		88.97541

				197.12		88.95781

				197.15		88.94901

				197.17		88.94021

				197.19		88.92262

				197.21		88.90502

				197.23		88.90502

				197.25		88.89622

				197.27		88.87862

				197.29		88.87422

				197.31		88.86103

				197.33		88.86103

				197.35		88.84783

				197.38		88.83463

				197.4		88.83023

				197.42		88.80824

				197.44		88.79064

				197.46		88.77304

				197.48		88.75984

				197.5		88.74225

				197.52		88.74225

				197.54		88.72905

				197.56		88.72025

				197.58		88.70705

				197.61		88.69385

				197.63		88.66306

				197.65		88.66306

				197.67		88.64106

				197.69		88.63226

				197.71		88.62347

				197.73		88.62787

				197.75		88.60587

				197.77		88.60147

				197.79		88.57947

				197.81		88.56188

				197.84		88.53988

				197.86		88.53108

				197.88		88.52228

				197.9		88.51788

				197.92		88.50908

				197.94		88.50469

				197.96		88.48709

				197.98		88.47829

				198		88.47389

				198.02		88.46069

				198.04		88.4431

				198.07		88.4431

				198.09		88.4299

				198.11		88.4123

				198.13		88.3947

				198.15		88.3859

				198.17		88.36391

				198.19		88.35511

				198.21		88.33751

				198.23		88.34191

				198.25		88.32871

				198.28		88.31992

				198.3		88.29792

				198.32		88.29792

				198.34		88.26712

				198.36		88.25833

				198.38		88.24073

				198.4		88.23193

				198.42		88.21873

				198.44		88.20553

				198.46		88.19234

				198.48		88.19234

				198.51		88.17914

				198.53		88.16594

				198.55		88.15274

				198.57		88.13955

				198.59		88.12635

				198.61		88.10435

				198.63		88.09115

				198.65		88.08235

				198.67		88.06916

				198.69		88.05596

				198.71		88.05156

				198.74		88.04276

				198.76		88.03396

				198.78		88.02516

				198.8		88.00757

				198.82		87.98997

				198.84		87.98117

				198.86		87.96357

				198.88		87.94158

				198.9		87.93718

				198.92		87.91518

				198.94		87.89758

				198.97		87.89758

				198.99		87.88439

				199.01		87.86679

				199.03		87.86239

				199.05		87.84479

				199.07		87.814

				199.09		87.8096

				199.11		87.792

				199.13		87.7876

				199.15		87.77001

				199.18		87.77001

				199.2		87.75681

				199.22		87.74801

				199.24		87.72601

				199.26		87.73041

				199.28		87.71282

				199.3		87.69962

				199.32		87.68642

				199.34		87.68202

				199.36		87.65562

				199.38		87.64243

				199.41		87.61603

				199.43		87.61603

				199.45		87.59403

				199.47		87.58964

				199.49		87.57644

				199.51		87.58964

				199.53		87.56764

				199.55		87.56324

				199.57		87.54124

				199.59		87.52805

				199.61		87.50165

				199.64		87.49285

				199.66		87.47525

				199.68		87.47525

				199.7		87.46206

				199.72		87.44446

				199.74		87.43126

				199.76		87.41806

				199.78		87.40487

				199.8		87.38727

				199.82		87.37847

				199.85		87.36527

				199.87		87.35207

				199.89		87.33448

				199.91		87.32128

				199.93		87.31688

				199.95		87.30368

				199.97		87.29488

				199.99		87.27729

				200.01		87.27289

				200.03		87.25529

				200.05		87.24649

				200.08		87.2245

				200.1		87.2157

				200.12		87.1981

				200.14		87.1849

				200.16		87.1673

				200.18		87.16291

				200.2		87.14971

				200.22		87.14971

				200.24		87.13651

				200.26		87.13211

				200.28		87.11451

				200.31		87.11451

				200.33		87.09692

				200.35		87.08812

				200.37		87.07492

				200.39		87.06172

				200.41		87.04852

				200.43		87.03973

				200.45		87.03093

				200.47		87.03093

				200.49		87.01333

				200.51		87.00453

				200.54		86.98693

				200.56		86.96934

				200.58		86.95174

				200.6		86.93854

				200.62		86.92534

				200.64		86.92094

				200.66		86.90775

				200.68		86.89455

				200.7		86.88135

				200.72		86.86375

				200.74		86.84616

				200.77		86.84176

				200.79		86.82856

				200.81		86.82856

				200.83		86.81536

				200.85		86.80656

				200.87		86.78897

				200.89		86.77137

				200.91		86.74937

				200.93		86.73618

				200.95		86.71858

				200.97		86.71418

				201		86.70978

				201.02		86.69658

				201.04		86.69218

				201.06		86.68338

				201.08		86.67019

				201.1		86.65699

				201.12		86.63939

				201.14		86.62179

				201.16		86.613

				201.18		86.5954

				201.21		86.5866

				201.23		86.5778

				201.25		86.569

				201.27		86.5558

				201.29		86.54701

				201.31		86.52501

				201.33		86.51181

				201.35		86.50301

				201.37		86.48982

				201.39		86.46782

				201.41		86.45902

				201.44		86.44582

				201.46		86.42383

				201.48		86.41943

				201.5		86.41503

				201.52		86.40183

				201.54		86.39743

				201.56		86.38863

				201.58		86.37543

				201.6		86.36224

				201.62		86.35344

				201.65		86.34024

				201.67		86.32264

				201.69		86.30505

				201.71		86.29625

				201.73		86.29185

				201.75		86.27425

				201.77		86.26985

				201.79		86.25225

				201.81		86.23466

				201.83		86.21266

				201.85		86.19946

				201.88		86.19066

				201.9		86.18627

				201.92		86.16867

				201.94		86.16427

				201.96		86.15107

				201.98		86.13347

				202		86.11588

				202.02		86.10708

				202.04		86.09388

				202.06		86.08948

				202.08		86.08068

				202.11		86.07188

				202.13		86.06309

				202.15		86.05429

				202.17		86.03229

				202.19		86.01469

				202.21		86.0015

				202.23		85.9839

				202.25		85.9707

				202.27		85.9575

				202.29		85.9531

				202.32		85.9531

				202.34		85.93551

				202.36		85.92231

				202.38		85.91351

				202.4		85.90471

				202.42		85.88272

				202.44		85.87392

				202.46		85.86072

				202.48		85.86072

				202.5		85.84312

				202.52		85.82552

				202.55		85.81673

				202.57		85.80353

				202.59		85.77713

				202.61		85.76393

				202.63		85.74634

				202.65		85.73754

				202.67		85.71994

				202.69		85.70674

				202.71		85.69355

				202.73		85.68475

				202.76		85.67155

				202.78		85.66715

				202.8		85.65835

				202.82		85.64955

				202.84		85.64515

				202.86		85.63636

				202.88		85.61876

				202.9		85.60996

				202.92		85.59676

				202.94		85.57477

				202.96		85.56597

				202.99		85.55277

				203.01		85.53077

				203.03		85.51758

				203.05		85.50438

				203.07		85.49558

				203.09		85.48238

				203.11		85.46918

				203.13		85.46478

				203.15		85.46038

				203.17		85.44279

				203.2		85.43839

				203.22		85.42959

				203.24		85.42079

				203.26		85.40319

				203.28		85.3856

				203.3		85.3768

				203.32		85.3636

				203.34		85.3548

				203.36		85.33281

				203.38		85.32841

				203.4		85.31521

				203.43		85.30641

				203.45		85.28881

				203.47		85.28441

				203.49		85.27122

				203.51		85.24922

				203.53		85.22722

				203.55		85.22722

				203.57		85.21842

				203.59		85.20523

				203.61		85.20963

				203.64		85.20523

				203.66		85.18323

				203.68		85.17883

				203.7		85.16563

				203.72		85.14804

				203.74		85.13484

				203.76		85.13044

				203.78		85.11724

				203.8		85.11724

				203.82		85.10844

				203.84		85.09524

				203.87		85.07765

				203.89		85.06005

				203.91		85.04245

				203.93		85.03365

				203.95		85.01606

				203.97		85.00286

				203.99		84.99406

				204.01		84.97646

				204.03		84.95887

				204.05		84.95007

				204.08		84.93247

				204.1		84.92367

				204.12		84.91487

				204.14		84.90168

				204.16		84.89288

				204.18		84.88408

				204.2		84.87088

				204.22		84.86648

				204.24		84.85328

				204.26		84.84888

				204.28		84.84009

				204.31		84.82689

				204.33		84.82249

				204.35		84.81809

				204.37		84.80049

				204.39		84.79169

				204.41		84.78729

				204.43		84.7741

				204.45		84.7565

				204.47		84.7477

				204.49		84.7301

				204.51		84.72131

				204.54		84.70371

				204.56		84.69931

				204.58		84.69051

				204.6		84.69051

				204.62		84.66412

				204.64		84.65972

				204.66		84.63332

				204.68		84.62452

				204.7		84.59813

				204.72		84.59813

				204.74		84.58493

				204.77		84.58933

				204.79		84.57173

				204.81		84.56733

				204.83		84.55413

				204.85		84.54094

				204.87		84.53214

				204.89		84.52334

				204.91		84.50134

				204.93		84.49694

				204.95		84.48814

				204.98		84.47495

				205		84.46615

				205.02		84.46175

				205.04		84.44415

				205.06		84.43535

				205.08		84.42215

				205.1		84.41336

				205.12		84.40016

				205.14		84.38696

				205.16		84.37816

				205.18		84.37376

				205.21		84.36056

				205.23		84.35617

				205.25		84.34297

				205.27		84.33417

				205.29		84.31657

				205.31		84.31217

				205.33		84.29897

				205.35		84.29897

				205.37		84.29018

				205.39		84.28578

				205.42		84.27698

				205.44		84.25938

				205.46		84.24618

				205.48		84.23739

				205.5		84.21979

				205.52		84.20219

				205.54		84.19779

				205.56		84.18019

				205.58		84.167

				205.6		84.1582

				205.62		84.1582

				205.65		84.1494

				205.67		84.1362

				205.69		84.1274

				205.71		84.1186

				205.73		84.10101

				205.75		84.09661

				205.77		84.09221

				205.79		84.08341

				205.81		84.07461

				205.83		84.05701

				205.86		84.03942

				205.88		84.03062

				205.9		84.02182

				205.92		84.00862

				205.94		84.00422

				205.96		83.99103

				205.98		83.97783

				206		83.97343

				206.02		83.96463

				206.04		83.95583

				206.06		83.95583

				206.09		83.93823

				206.11		83.92064

				206.13		83.91184

				206.15		83.89864

				206.17		83.87224

				206.19		83.87224

				206.21		83.85465

				206.23		83.84585

				206.25		83.84145

				206.27		83.84145

				206.3		83.83265

				206.32		83.83265

				206.34		83.81945

				206.36		83.80626

				206.38		83.79746

				206.4		83.78426

				206.42		83.77986

				206.44		83.77106

				206.46		83.75786

				206.48		83.74467

				206.5		83.72707

				206.53		83.72267

				206.55		83.71827

				206.57		83.71387

				206.59		83.70067

				206.61		83.69627

				206.63		83.67428

				206.65		83.66108

				206.67		83.64788

				206.69		83.64788

				206.71		83.63028

				206.74		83.62149

				206.76		83.60389

				206.78		83.60389

				206.8		83.58629

				206.82		83.58189

				206.84		83.5643

				206.86		83.56869

				206.88		83.5467

				206.9		83.5379

				206.92		83.5247

				206.94		83.5203

				206.97		83.50271

				206.99		83.48951

				207.01		83.46311

				207.03		83.45431

				207.05		83.43672

				207.07		83.42792

				207.09		83.41472

				207.11		83.41472

				207.13		83.41472

				207.15		83.40592

				207.17		83.38832

				207.2		83.38832

				207.22		83.37073

				207.24		83.35313

				207.26		83.33553

				207.28		83.33553

				207.3		83.32234

				207.32		83.31354

				207.34		83.29154

				207.36		83.28714

				207.38		83.28274

				207.41		83.26954

				207.43		83.24755

				207.45		83.25635

				207.47		83.23875

				207.49		83.22555

				207.51		83.20355

				207.53		83.20355

				207.55		83.18156

				207.57		83.18156

				207.59		83.15516

				207.61		83.15956

				207.64		83.15076

				207.66		83.14196

				207.68		83.12437

				207.7		83.12437

				207.72		83.10677

				207.74		83.09797

				207.76		83.08477

				207.78		83.07598

				207.8		83.06718

				207.82		83.06278

				207.85		83.05398

				207.87		83.05398

				207.89		83.04078

				207.91		83.03198

				207.93		83.02318

				207.95		83.00119

				207.97		82.99679

				207.99		82.99239

				208.01		82.97479

				208.03		82.96159

				208.05		82.9528

				208.08		82.9352

				208.1		82.9176

				208.12		82.9088

				208.14		82.9044

				208.16		82.89561

				208.18		82.87801

				208.2		82.87801

				208.22		82.86921

				208.24		82.86041

				208.26		82.84281

				208.29		82.84721

				208.31		82.82522

				208.33		82.81202

				208.35		82.79882

				208.37		82.79002

				208.39		82.78122

				208.41		82.77243

				208.43		82.75923

				208.45		82.75043

				208.47		82.73283

				208.49		82.71523

				208.52		82.70204

				208.54		82.69764

				208.56		82.68884

				208.58		82.68444

				208.6		82.67564

				208.62		82.66244

				208.64		82.65364

				208.66		82.63165

				208.68		82.61405

				208.7		82.60525

				208.73		82.60085

				208.75		82.58766

				208.77		82.56566

				208.79		82.56126

				208.81		82.54806

				208.83		82.53047

				208.85		82.50847

				208.87		82.50407

				208.89		82.49087

				208.91		82.47327

				208.93		82.46888

				208.96		82.46448

				208.98		82.45568

				209		82.44688

				209.02		82.43368

				209.04		82.42048

				209.06		82.41168

				209.08		82.39409

				209.1		82.37649

				209.12		82.37649

				209.14		82.35449

				209.17		82.3413

				209.19		82.3281

				209.21		82.3237

				209.23		82.3061

				209.25		82.3061

				209.27		82.28411

				209.29		82.27091

				209.31		82.26651

				209.33		82.25771

				209.35		82.25331

				209.37		82.25331

				209.4		82.24011

				209.42		82.22691

				209.44		82.21812

				209.46		82.19612

				209.48		82.18732

				209.5		82.16972

				209.52		82.15653

				209.54		82.13893

				209.56		82.13453

				209.58		82.12133

				209.61		82.10813

				209.63		82.09494

				209.65		82.08614

				209.67		82.07734

				209.69		82.06414

				209.71		82.05534

				209.73		82.05534

				209.75		82.04215

				209.77		82.02895

				209.79		82.01575

				209.81		82.00695

				209.84		81.99375

				209.86		81.98056

				209.88		81.96736

				209.9		81.96736

				209.92		81.95416

				209.94		81.94096

				209.96		81.92776

				209.98		81.91457

				210		81.89697

				210.02		81.88377

				210.05		81.85738

				210.07		81.84858

				210.09		81.83538

				210.11		81.81778

				210.13		81.80458

				210.15		81.80018

				210.17		81.78259

				210.19		81.77379

				210.21		81.76499

				210.23		81.75619

				210.25		81.74739

				210.28		81.7342

				210.3		81.7166

				210.32		81.7166

				210.34		81.699

				210.36		81.6858

				210.38		81.66821

				210.4		81.65941

				210.42		81.64621

				210.44		81.62861

				210.46		81.61102

				210.49		81.61102

				210.51		81.59782

				210.53		81.57582

				210.55		81.56702

				210.57		81.56262

				210.59		81.54503

				210.61		81.53183

				210.63		81.52743

				210.65		81.51863

				210.67		81.50103

				210.69		81.47904

				210.72		81.47464

				210.74		81.45264

				210.76		81.43944

				210.78		81.43065

				210.8		81.42625

				210.82		81.40865

				210.84		81.39985

				210.86		81.39545

				210.88		81.37785

				210.9		81.36466

				210.93		81.35146

				210.95		81.33386

				210.97		81.31186

				210.99		81.30747

				211.01		81.29427

				211.03		81.28547

				211.05		81.27227

				211.07		81.26787

				211.09		81.25467

				211.11		81.24148

				211.14		81.21948

				211.16		81.21508

				211.18		81.19308

				211.2		81.17549

				211.22		81.15789

				211.24		81.14469

				211.26		81.1271

				211.28		81.1183

				211.3		81.0963

				211.32		81.0963

				211.34		81.0875

				211.37		81.0743

				211.39		81.0699

				211.41		81.0743

				211.43		81.05231

				211.45		81.03911

				211.47		81.02151

				211.49		81.00831

				211.51		80.99072

				211.53		80.98192

				211.55		80.96872

				211.58		80.96432

				211.6		80.94233

				211.62		80.92913

				211.64		80.91593

				211.66		80.90273

				211.68		80.88074

				211.7		80.87194

				211.72		80.86314

				211.74		80.86754

				211.76		80.85874

				211.79		80.85434

				211.81		80.84114

				211.83		80.83234

				211.85		80.80155

				211.87		80.78835

				211.89		80.76635

				211.91		80.75756

				211.93		80.73556

				211.95		80.71356

				211.97		80.69597

				211.99		80.69597

				212.02		80.67837

				212.04		80.66517

				212.06		80.65197

				212.08		80.64757

				212.1		80.62998

				212.12		80.60798

				212.14		80.59918

				212.16		80.59478

				212.18		80.58158

				212.2		80.56839

				212.23		80.55519

				212.25		80.53319

				212.27		80.5156

				212.29		80.498

				212.31		80.4892

				212.33		80.476

				212.35		80.4716

				212.37		80.45401

				212.39		80.44081

				212.41		80.43201

				212.44		80.41881

				212.46		80.41441

				212.48		80.40121

				212.5		80.37922

				212.52		80.36162

				212.54		80.35282

				212.56		80.32203

				212.58		80.31763

				212.6		80.30883

				212.62		80.30003

				212.64		80.28243

				212.67		80.28243

				212.69		80.25604

				212.71		80.25164

				212.73		80.22964

				212.75		80.22524

				212.77		80.20325

				212.79		80.19445

				212.81		80.17245

				212.83		80.17245

				212.85		80.14606

				212.88		80.13286

				212.9		80.11086

				212.92		80.10206

				212.94		80.07567

				212.96		80.06687

				212.98		80.04487

				213		80.03607

				213.02		80.02288

				213.04		80.01848

				213.06		80.00528

				213.08		80.00088

				213.11		79.98768

				213.13		79.97888

				213.15		79.95689

				213.17		79.93489

				213.19		79.92609

				213.21		79.91729

				213.23		79.8865

				213.25		79.8865

				213.27		79.8689

				213.29		79.8601

				213.32		79.82931

				213.34		79.82051

				213.36		79.79851

				213.38		79.79851

				213.4		79.77212

				213.42		79.77652

				213.44		79.76332

				213.46		79.75452

				213.48		79.73692

				213.5		79.72812

				213.52		79.71053

				213.55		79.71053

				213.57		79.68413

				213.59		79.67973

				213.61		79.65774

				213.63		79.64454

				213.65		79.61814

				213.67		79.61814

				213.69		79.58735

				213.71		79.57415

				213.73		79.56095

				213.76		79.55655

				213.78		79.53896

				213.8		79.53456

				213.82		79.52136

				213.84		79.51256

				213.86		79.49056

				213.88		79.46857

				213.9		79.45097

				213.92		79.43337

				213.94		79.41138

				213.97		79.41138

				213.99		79.39818

				214.01		79.38498

				214.03		79.36298

				214.05		79.34979

				214.07		79.32339

				214.09		79.31899

				214.11		79.30139

				214.13		79.2882

				214.15		79.2794

				214.17		79.275

				214.2		79.253

				214.22		79.2398

				214.24		79.22661

				214.26		79.21341

				214.28		79.19581

				214.3		79.16502

				214.32		79.15182

				214.34		79.13862

				214.36		79.12102

				214.38		79.11662

				214.41		79.11662

				214.43		79.10343

				214.45		79.08583

				214.47		79.06823

				214.49		79.05503

				214.51		79.03304

				214.53		79.02424

				214.55		79.01104

				214.57		78.99784

				214.59		78.97145

				214.62		78.95825

				214.64		78.94065

				214.66		78.91866

				214.68		78.90106

				214.7		78.89226

				214.72		78.87466

				214.74		78.85267

				214.76		78.83507

				214.78		78.82187

				214.8		78.81307

				214.83		78.79548

				214.85		78.78228

				214.87		78.78228

				214.89		78.76468

				214.91		78.75588

				214.93		78.74269

				214.95		78.72069

				214.97		78.69869

				214.99		78.69429

				215.01		78.6635

				215.03		78.6503

				215.06		78.6459

				215.08		78.6371

				215.1		78.61511

				215.12		78.60631

				215.14		78.58431

				215.16		78.56672

				215.18		78.54472

				215.2		78.52712

				215.22		78.51392

				215.24		78.50952

				215.27		78.47873

				215.29		78.46993

				215.31		78.45233

				215.33		78.43914

				215.35		78.41274

				215.37		78.40834

				215.39		78.39074

				215.41		78.37755

				215.43		78.35115

				215.45		78.34675

				215.47		78.32915

				215.5		78.31596

				215.52		78.29836

				215.54		78.28516

				215.56		78.26756

				215.58		78.24997

				215.6		78.23677

				215.62		78.21917

				215.64		78.20597

				215.66		78.19278

				215.68		78.17078

				215.71		78.15758

				215.73		78.14438

				215.75		78.13559

				215.77		78.11799

				215.79		78.10919

				215.81		78.09599

				215.83		78.08279

				215.85		78.0608

				215.87		78.0476

				215.89		78.03

				215.92		78.01241

				215.94		77.99041

				215.96		77.97721

				215.98		77.95522

				216		77.94202

				216.02		77.92442

				216.04		77.91122

				216.06		77.89363

				216.08		77.89363

				216.1		77.87163

				216.13		77.85403

				216.15		77.83204

				216.17		77.81444

				216.19		77.77924

				216.21		77.77045

				216.23		77.76165

				216.25		77.75285

				216.27		77.73965

				216.29		77.73525

				216.31		77.71765

				216.33		77.70006

				216.36		77.68686

				216.38		77.66926

				216.4		77.65167

				216.42		77.62967

				216.44		77.62087

				216.46		77.60327

				216.48		77.59008

				216.5		77.56808

				216.52		77.55928

				216.54		77.53728

				216.57		77.51529

				216.59		77.49329

				216.61		77.48889

				216.63		77.4669

				216.65		77.4493

				216.67		77.4361

				216.69		77.4141

				216.71		77.39651

				216.73		77.37891

				216.75		77.37011

				216.78		77.35251

				216.8		77.34372

				216.82		77.32612

				216.84		77.30852

				216.86		77.28653

				216.88		77.26453

				216.9		77.24253

				216.92		77.22933

				216.94		77.21614

				216.96		77.20294

				216.99		77.18094

				217.01		77.17654

				217.03		77.15015

				217.05		77.13255

				217.07		77.11055

				217.09		77.11495

				217.11		77.09736

				217.13		77.09296

				217.15		77.08416

				217.17		77.07096

				217.19		77.05336

				217.22		77.03577

				217.24		77.01817

				217.26		76.99617

				217.28		76.96978

				217.3		76.95218

				217.32		76.93018

				217.34		76.90819

				217.36		76.89059

				217.38		76.87739

				217.4		76.8554

				217.43		76.8378

				217.45		76.8246

				217.47		76.807

				217.49		76.78941

				217.51		76.78061

				217.53		76.77621

				217.55		76.75861

				217.57		76.73662

				217.59		76.71462

				217.61		76.69702

				217.64		76.67503

				217.66		76.65303

				217.68		76.64863

				217.7		76.63543

				217.72		76.61783

				217.74		76.59144

				217.76		76.58264

				217.78		76.55624

				217.8		76.53865

				217.82		76.51665

				217.84		76.50785

				217.87		76.49026

				217.89		76.48146

				217.91		76.45506

				217.93		76.45506

				217.95		76.43746

				217.97		76.41107

				217.99		76.39347

				218.01		76.38027

				218.03		76.35388

				218.05		76.33628

				218.08		76.31428

				218.1		76.30549

				218.12		76.28349

				218.14		76.26149

				218.16		76.2439

				218.18		76.2307

				218.2		76.2087

				218.22		76.1911

				218.24		76.17351

				218.26		76.16031

				218.29		76.14271

				218.31		76.12951

				218.33		76.10752

				218.35		76.08552

				218.37		76.06353

				218.39		76.05033

				218.41		76.01953

				218.43		76.01513

				218.45		76.00633

				218.47		75.99314

				218.5		75.97554

				218.52		75.96674

				218.54		75.94035

				218.56		75.92275

				218.58		75.90075

				218.6		75.87876

				218.62		75.86556

				218.64		75.85236

				218.66		75.82157

				218.68		75.80837

				218.71		75.78197

				218.73		75.76437

				218.75		75.74678

				218.77		75.73798

				218.79		75.71598

				218.81		75.70718

				218.83		75.68519

				218.85		75.66759

				218.87		75.65879

				218.89		75.64559

				218.92		75.6324

				218.94		75.6192

				218.96		75.6016

				218.98		75.5796

				219		75.55761

				219.02		75.53561

				219.04		75.51802

				219.06		75.50042

				219.08		75.47402

				219.1		75.47402

				219.13		75.45643

				219.15		75.43443

				219.17		75.41243

				219.19		75.40363

				219.21		75.35964

				219.23		75.34644

				219.25		75.32445

				219.27		75.31125

				219.29		75.29805

				219.31		75.28925

				219.34		75.27605

				219.36		75.26726

				219.38		75.24966

				219.4		75.22766

				219.42		75.20127

				219.44		75.17927

				219.46		75.15727

				219.48		75.13088

				219.5		75.11768

				219.52		75.09568

				219.55		75.08249

				219.57		75.06049

				219.59		75.04729

				219.61		75.0209

				219.63		75.0077

				219.65		74.9813

				219.67		74.96371

				219.69		74.93731

				219.71		74.92411

				219.74		74.90212

				219.76		74.89772

				219.78		74.87572

				219.8		74.86692

				219.82		74.84493

				219.84		74.82733

				219.86		74.79213

				219.88		74.78773

				219.9		74.77014

				219.92		74.74814

				219.95		74.73494

				219.97		74.72175

				219.99		74.69535

				220.01		74.68655

				220.03		74.66456

				220.05		74.64256

				220.07		74.62056

				220.09		74.60297

				220.11		74.56777

				220.13		74.55457

				220.16		74.53698

				220.18		74.51058

				220.2		74.49738

				220.22		74.47539

				220.24		74.45779

				220.26		74.44019

				220.28		74.4182

				220.3		74.405

				220.32		74.3918

				220.34		74.3698

				220.37		74.34341

				220.39		74.33901

				220.41		74.30821

				220.43		74.29062

				220.45		74.27302

				220.47		74.25982

				220.49		74.23343

				220.51		74.22023

				220.53		74.20263

				220.56		74.18943

				220.58		74.16304

				220.6		74.14984

				220.62		74.11904

				220.64		74.10585

				220.66		74.08385

				220.68		74.06625

				220.7		74.04866

				220.72		74.03546

				220.74		74.01346

				220.77		73.98267

				220.79		73.96507

				220.81		73.93867

				220.83		73.90788

				220.85		73.88588

				220.87		73.86389

				220.89		73.85069

				220.91		73.82869

				220.93		73.8023

				220.95		73.7935

				220.98		73.7715

				221		73.74511

				221.02		73.73191

				221.04		73.73191

				221.06		73.70551

				221.08		73.69231

				221.1		73.67472

				221.12		73.65272

				221.14		73.63072

				221.16		73.60873

				221.19		73.58673

				221.21		73.56474

				221.23		73.55154

				221.25		73.52514

				221.27		73.51194

				221.29		73.48995

				221.31		73.46795

				221.33		73.44156

				221.35		73.43276

				221.38		73.41076

				221.4		73.41076

				221.42		73.39316

				221.44		73.37557

				221.46		73.35357

				221.48		73.33157

				221.5		73.30078

				221.52		73.27878

				221.54		73.26119

				221.56		73.24799

				221.59		73.23039

				221.61		73.20839

				221.63		73.1908

				221.65		73.16

				221.67		73.12481

				221.69		73.09841

				221.71		73.07642

				221.73		73.05442

				221.75		73.04122

				221.77		73.02362

				221.8		73.00603

				221.82		72.98843

				221.84		72.96643

				221.86		72.94884

				221.88		72.94004

				221.9		72.91804

				221.92		72.89605

				221.94		72.87845

				221.96		72.84325

				221.99		72.82566

				222.01		72.80366

				222.03		72.78166

				222.05		72.75527

				222.07		72.74207

				222.09		72.71128

				222.11		72.69808

				222.13		72.68048

				222.15		72.66288

				222.17		72.64089

				222.2		72.61889

				222.22		72.59689

				222.24		72.5749

				222.26		72.5529

				222.28		72.5353

				222.3		72.51331

				222.32		72.50011

				222.34		72.47811

				222.36		72.45612

				222.38		72.43412

				222.41		72.41652

				222.43		72.39013

				222.45		72.37253

				222.47		72.35493

				222.49		72.33294

				222.51		72.31534

				222.53		72.29774

				222.55		72.27135

				222.57		72.25815

				222.6		72.23615

				222.62		72.20976

				222.64		72.19216

				222.66		72.17896

				222.68		72.15257

				222.7		72.14377

				222.72		72.12177

				222.74		72.09538

				222.76		72.06898

				222.78		72.05138

				222.81		72.02059

				222.83		72.00299

				222.85		71.98539

				222.87		71.959

				222.89		71.937

				222.91		71.91501

				222.93		71.88861

				222.95		71.86221

				222.97		71.84462

				223		71.80942

				223.02		71.79183

				223.04		71.76983

				223.06		71.74783

				223.08		71.73464

				223.1		71.72584

				223.12		71.70384

				223.14		71.67305

				223.16		71.65105

				223.18		71.62465

				223.21		71.60266

				223.23		71.58506

				223.25		71.56746

				223.27		71.54547

				223.29		71.52347

				223.31		71.49707

				223.33		71.47508

				223.35		71.44868

				223.37		71.43548

				223.4		71.41349

				223.42		71.40029

				223.44		71.37389

				223.46		71.3519

				223.48		71.3299

				223.5		71.3123

				223.52		71.28591

				223.54		71.27271

				223.56		71.24632

				223.59		71.21992

				223.61		71.19352

				223.63		71.18033

				223.65		71.14073

				223.67		71.12754

				223.69		71.10554

				223.71		71.08354

				223.73		71.05275

				223.75		71.03955

				223.77		71.01315

				223.8		70.99116

				223.82		70.96916

				223.84		70.95156

				223.86		70.93397

				223.88		70.91637

				223.9		70.89877

				223.92		70.88557

				223.94		70.85918

				223.96		70.82838

				223.99		70.80199

				224.01		70.77999

				224.03		70.7536

				224.05		70.7404

				224.07		70.7184

				224.09		70.70081

				224.11		70.67441

				224.13		70.65681

				224.15		70.63042

				224.17		70.60842

				224.2		70.57763

				224.22		70.56443

				224.24		70.52923

				224.26		70.51604

				224.28		70.48964

				224.3		70.47204

				224.32		70.43685

				224.34		70.41925

				224.36		70.39286

				224.39		70.37086

				224.41		70.34886

				224.43		70.33566

				224.45		70.31367

				224.47		70.30047

				224.49		70.27408

				224.51		70.25648

				224.53		70.23008

				224.55		70.20369

				224.57		70.17729

				224.6		70.15529

				224.62		70.1289

				224.64		70.1113

				224.66		70.0981

				224.68		70.07611

				224.7		70.06291

				224.72		70.02332

				224.74		70.00132

				224.76		69.97932

				224.79		69.95293

				224.81		69.92213

				224.83		69.91773

				224.85		69.88254

				224.87		69.86054

				224.89		69.83855

				224.91		69.81215

				224.93		69.78576

				224.95		69.76816

				224.97		69.74176

				225		69.72417

				225.02		69.69777

				225.04		69.67137

				225.06		69.65818

				225.08		69.63178

				225.1		69.60538

				225.12		69.59659

				225.14		69.56579

				225.16		69.54379

				225.19		69.5174

				225.21		69.4954

				225.23		69.46901

				225.25		69.45141

				225.27		69.42062

				225.29		69.39862

				225.31		69.37222

				225.33		69.34583

				225.35		69.31943

				225.37		69.29744

				225.4		69.27104

				225.42		69.25784

				225.44		69.22705

				225.46		69.20945

				225.48		69.18305

				225.5		69.16986

				225.52		69.13906

				225.54		69.11706

				225.56		69.09507

				225.58		69.07747

				225.61		69.04668

				225.63		69.02908

				225.65		69.00708

				225.67		68.97629

				225.69		68.94989

				225.71		68.93669

				225.73		68.9015

				225.75		68.8883

				225.77		68.85311

				225.79		68.83551

				225.82		68.80032

				225.84		68.77832

				225.86		68.74313

				225.88		68.72553

				225.9		68.70353

				225.92		68.68594

				225.94		68.66394

				225.96		68.65074

				225.98		68.61995

				226		68.59795

				226.03		68.56715

				226.05		68.54076

				226.07		68.51876

				226.09		68.49237

				226.11		68.46597

				226.13		68.44398

				226.15		68.42638

				226.17		68.39998

				226.19		68.38239

				226.21		68.36039

				226.24		68.33399

				226.26		68.3076

				226.28		68.2768

				226.3		68.25921

				226.32		68.23721

				226.34		68.21081

				226.36		68.18882

				226.38		68.16242

				226.4		68.14042

				226.42		68.10963

				226.45		68.08763

				226.47		68.06124

				226.49		68.03484

				226.51		68.00845

				226.53		67.99085

				226.55		67.96885

				226.57		67.93806

				226.59		67.92046

				226.61		67.88967

				226.63		67.86327

				226.66		67.84127

				226.68		67.81928

				226.7		67.79288

				226.72		67.76649

				226.74		67.75329

				226.76		67.71369

				226.78		67.6917

				226.8		67.6697

				226.82		67.64331

				226.84		67.60811

				226.87		67.59491

				226.89		67.56412

				226.91		67.53332

				226.93		67.51133

				226.95		67.49373

				226.97		67.46294

				226.99		67.43654

				227.01		67.41454

				227.03		67.39255

				227.05		67.36175

				227.08		67.33096

				227.1		67.31336

				227.12		67.29136

				227.14		67.26497

				227.16		67.23857

				227.18		67.21218

				227.2		67.18578

				227.22		67.15939

				227.24		67.12859

				227.26		67.10659

				227.29		67.0846

				227.31		67.0582

				227.33		67.03621

				227.35		67.01421

				227.37		66.98341

				227.39		66.95702

				227.41		66.92622

				227.43		66.89543

				227.45		66.86903

				227.48		66.83824

				227.5		66.81184

				227.52		66.78985

				227.54		66.75905

				227.56		66.73706

				227.58		66.71506

				227.6		66.69306

				227.62		66.66227

				227.64		66.64027

				227.66		66.60508

				227.69		66.58748

				227.71		66.56108

				227.73		66.54349

				227.75		66.51269

				227.77		66.49949

				227.79		66.4599

				227.81		66.4379

				227.83		66.40711

				227.85		66.38951

				227.87		66.35872

				227.9		66.34112

				227.92		66.29713

				227.94		66.28833

				227.96		66.24434

				227.98		66.22234

				228		66.18715

				228.02		66.17395

				228.04		66.12995

				228.06		66.10796

				228.08		66.07276

				228.11		66.05517

				228.13		66.02437

				228.15		66.00677

				228.17		65.97598

				228.19		65.95838

				228.21		65.92759

				228.23		65.90559

				228.25		65.8748

				228.27		65.8572

				228.29		65.82201

				228.32		65.80001

				228.34		65.77801

				228.36		65.75162

				228.38		65.72522

				228.4		65.71202

				228.42		65.68563

				228.44		65.65043

				228.46		65.63284

				228.48		65.60204

				228.5		65.56245

				228.52		65.54045

				228.55		65.51845

				228.57		65.48766

				228.59		65.45687

				228.61		65.43487

				228.63		65.40407

				228.65		65.37328

				228.67		65.33369

				228.69		65.31609

				228.71		65.29849

				228.73		65.27649

				228.76		65.2457

				228.78		65.2281

				228.8		65.20171

				228.82		65.17091

				228.84		65.14892

				228.86		65.12252

				228.88		65.10052

				228.9		65.07413

				228.92		65.03014

				228.94		64.99494

				228.97		64.96855

				228.99		64.93335

				229.01		64.90696

				229.03		64.88936

				229.05		64.86736

				229.07		64.84097

				229.09		64.81457

				229.11		64.77938

				229.13		64.75738

				229.15		64.73098

				229.18		64.69579

				229.2		64.66939

				229.22		64.6518

				229.24		64.621

				229.26		64.59461

				229.28		64.56821

				229.3		64.54182

				229.32		64.51102

				229.34		64.48023

				229.36		64.45823

				229.39		64.43623

				229.41		64.40544

				229.43		64.37904

				229.45		64.35265

				229.47		64.32185

				229.49		64.29546

				229.51		64.26466

				229.53		64.24266

				229.55		64.21627

				229.57		64.18547

				229.6		64.15028

				229.62		64.13268

				229.64		64.10189

				229.66		64.07549

				229.68		64.0447

				229.7		64.0183

				229.72		63.98751

				229.74		63.95671

				229.76		63.93471

				229.78		63.90832

				229.81		63.87752

				229.83		63.84673

				229.85		63.82473

				229.87		63.78514

				229.89		63.76754

				229.91		63.74115

				229.93		63.71475

				229.95		63.68396

				229.97		63.66196

				229.99		63.62677

				230.01		63.58717

				230.04		63.56078

				230.06		63.53438

				230.08		63.50359

				230.1		63.47719

				230.12		63.45959

				230.14		63.4332

				230.16		63.3936

				230.18		63.35841

				230.2		63.33641

				230.22		63.30122

				230.25		63.27482

				230.27		63.24843

				230.29		63.21323

				230.31		63.17364

				230.33		63.14284

				230.35		63.11645

				230.37		63.08125

				230.39		63.06806

				230.41		63.04166

				230.43		63.01966

				230.46		62.98887

				230.48		62.97127

				230.5		62.94488

				230.52		62.90968

				230.54		62.88769

				230.56		62.86569

				230.58		62.83929

				230.6		62.8085

				230.62		62.7953

				230.64		62.75571

				230.67		62.72051

				230.69		62.68092

				230.71		62.65013

				230.73		62.61933

				230.75		62.58414

				230.77		62.55334

				230.79		62.54014

				230.81		62.51815

				230.83		62.47855

				230.85		62.44776

				230.87		62.42576

				230.9		62.39057

				230.92		62.35977

				230.94		62.32018

				230.96		62.29378

				230.98		62.26299

				231		62.22779

				231.02		62.1838

				231.04		62.1706

				231.06		62.14421

				231.08		62.11781

				231.11		62.07382

				231.13		62.06502

				231.15		62.02983

				231.17		62.00343

				231.19		61.96824

				231.21		61.95504

				231.23		61.91985

				231.25		61.88465

				231.27		61.84946

				231.29		61.82746

				231.31		61.80106

				231.34		61.76587

				231.36		61.73068

				231.38		61.70868

				231.4		61.67788

				231.42		61.64709

				231.44		61.61629

				231.46		61.5943

				231.48		61.5679

				231.5		61.53711

				231.52		61.50191

				231.55		61.47992

				231.57		61.45792

				231.59		61.42713

				231.61		61.38753

				231.63		61.36554

				231.65		61.33034

				231.67		61.29075

				231.69		61.25115

				231.71		61.23356

				231.73		61.19836

				231.75		61.17197

				231.78		61.14117

				231.8		61.11918

				231.82		61.08838

				231.84		61.05319

				231.86		61.01359

				231.88		60.9916

				231.9		60.9652

				231.92		60.93001

				231.94		60.90361

				231.96		60.87282

				231.99		60.84642

				232.01		60.81563

				232.03		60.78923

				232.05		60.76283

				232.07		60.73644

				232.09		60.70124

				232.11		60.67925

				232.13		60.63526

				232.15		60.60446

				232.17		60.57367

				232.2		60.53407

				232.22		60.50328

				232.24		60.48128

				232.26		60.45049

				232.28		60.42409

				232.3		60.3933

				232.32		60.3581

				232.34		60.32291

				232.36		60.29651

				232.38		60.25252

				232.4		60.22612

				232.43		60.18653

				232.45		60.15573

				232.47		60.11614

				232.49		60.08535

				232.51		60.05895

				232.53		60.02816

				232.55		59.99296

				232.57		59.97096

				232.59		59.94457

				232.61		59.90498

				232.64		59.87418

				232.66		59.85658

				232.68		59.81699

				232.7		59.79059

				232.72		59.773

				232.74		59.7378

				232.76		59.70261

				232.78		59.67621

				232.8		59.63662

				232.82		59.60143

				232.85		59.57503

				232.87		59.53984

				232.89		59.50464

				232.91		59.47825

				232.93		59.44745

				232.95		59.42105

				232.97		59.39466

				232.99		59.36386

				233.01		59.33747

				233.03		59.29788

				233.05		59.26268

				233.08		59.23189

				233.1		59.19229

				233.12		59.1527

				233.14		59.1263

				233.16		59.09111

				233.18		59.06031

				233.2		59.02512

				233.22		58.98993

				233.24		58.96793

				233.26		58.93713

				233.29		58.89754

				233.31		58.86675

				233.33		58.84915

				233.35		58.80516

				233.37		58.78316

				233.39		58.74797

				233.41		58.71277

				233.43		58.67758

				233.45		58.65118

				233.47		58.60719

				233.5		58.58959

				233.52		58.5588

				233.54		58.528

				233.56		58.48841

				233.58		58.46641

				233.6		58.42242

				233.62		58.38722

				233.64		58.35643

				233.66		58.33003

				233.68		58.29924

				233.71		58.27724

				233.73		58.23325

				233.75		58.21125

				233.77		58.16726

				233.79		58.14086

				233.81		58.09687

				233.83		58.07927

				233.85		58.03968

				233.87		58.00449

				233.89		57.97369

				233.92		57.9473

				233.94		57.9121

				233.96		57.88571

				233.98		57.85491

				234		57.81532

				234.02		57.77572

				234.04		57.74053

				234.06		57.68774

				234.08		57.66134

				234.1		57.62615

				234.12		57.58656

				234.15		57.55576

				234.17		57.53376

				234.19		57.48977

				234.21		57.45898

				234.23		57.43698

				234.25		57.40179

				234.27		57.37539

				234.29		57.34899

				234.31		57.3138

				234.33		57.28301

				234.36		57.25221

				234.38		57.21262

				234.4		57.17742

				234.42		57.13343

				234.44		57.10703

				234.46		57.07184

				234.48		57.04105

				234.5		57.02345

				234.52		56.99705

				234.54		56.95746

				234.57		56.91787

				234.59		56.88707

				234.61		56.84308

				234.63		56.80788

				234.65		56.76829

				234.67		56.75069

				234.69		56.7067

				234.71		56.67151

				234.73		56.64511

				234.75		56.61432

				234.77		56.57472

				234.8		56.54833

				234.82		56.52193

				234.84		56.48234

				234.86		56.45154

				234.88		56.42515

				234.9		56.38115

				234.92		56.34156

				234.94		56.31516

				234.96		56.27117

				234.98		56.24038

				235.01		56.20518

				235.03		56.16999

				235.05		56.13479

				235.07		56.1084

				235.09		56.06441

				235.11		56.03361

				235.13		55.99842

				235.15		55.96762

				235.17		55.93683

				235.19		55.90603

				235.22		55.86644

				235.24		55.83564

				235.26		55.80045

				235.28		55.76525

				235.3		55.73006

				235.32		55.69487

				235.34		55.65967

				235.36		55.62008

				235.38		55.58048

				235.4		55.54529

				235.42		55.5145

				235.45		55.4749

				235.47		55.44851

				235.49		55.41331

				235.51		55.37812

				235.53		55.34732

				235.55		55.30773

				235.57		55.26814

				235.59		55.23734

				235.61		55.20655

				235.63		55.17135

				235.66		55.13176

				235.68		55.09216

				235.7		55.06137

				235.72		55.01738

				235.74		54.97778

				235.76		54.95139

				235.78		54.92059

				235.8		54.8722

				235.82		54.8502

				235.84		54.81501

				235.87		54.77542

				235.89		54.74462

				235.91		54.71383

				235.93		54.67863

				235.95		54.64784

				235.97		54.61264

				235.99		54.56865

				236.01		54.53786

				236.03		54.49826

				236.05		54.45867

				236.07		54.42347

				236.1		54.39268

				236.12		54.36188

				236.14		54.33109

				236.16		54.30029

				236.18		54.2651

				236.2		54.22551

				236.22		54.19031

				236.24		54.15952

				236.26		54.11992

				236.28		54.08473

				236.31		54.05833

				236.33		54.02314

				236.35		53.98355

				236.37		53.94835

				236.39		53.91316

				236.41		53.86917

				236.43		53.83397

				236.45		53.78998

				236.47		53.75478

				236.49		53.71959

				236.51		53.69319

				236.54		53.6492

				236.56		53.61841

				236.58		53.58321

				236.6		53.54802

				236.62		53.50842

				236.64		53.46443

				236.66		53.42484

				236.68		53.38524

				236.7		53.34565

				236.72		53.31926

				236.75		53.28846

				236.77		53.26207

				236.79		53.23567

				236.81		53.19168

				236.83		53.14328

				236.85		53.10369

				236.87		53.0597

				236.89		53.01571

				236.91		52.98931

				236.93		52.94972

				236.95		52.91892

				236.98		52.88373

				237		52.85293

				237.02		52.81334

				237.04		52.77814

				237.06		52.72975

				237.08		52.69456

				237.1		52.65057

				237.12		52.61097

				237.14		52.56698

				237.16		52.54498

				237.19		52.50539

				237.21		52.47899

				237.23		52.4394

				237.25		52.413

				237.27		52.36901

				237.29		52.32942

				237.31		52.28982

				237.33		52.25463

				237.35		52.21064

				237.37		52.18424

				237.39		52.14905

				237.42		52.11385

				237.44		52.07866

				237.46		52.04346

				237.48		51.99947

				237.5		51.96428

				237.52		51.92468

				237.54		51.88949

				237.56		51.8499

				237.58		51.8147

				237.6		51.77511

				237.63		51.73552

				237.65		51.69152

				237.67		51.65633

				237.69		51.62553

				237.71		51.59034

				237.73		51.55514

				237.75		51.52435

				237.77		51.48036

				237.79		51.44076

				237.81		51.38797

				237.83		51.34838

				237.86		51.31318

				237.88		51.28239

				237.9		51.2384

				237.92		51.212

				237.94		51.18121

				237.96		51.14161

				237.98		51.09762

				238		51.06683

				238.02		51.03163

				238.04		50.99204

				238.07		50.95244

				238.09		50.92605

				238.11		50.88206

				238.13		50.84246

				238.15		50.80287

				238.17		50.77207

				238.19		50.72368

				238.21		50.69289

				238.23		50.64889

				238.25		50.6181

				238.28		50.57851

				238.3		50.54331

				238.32		50.49932

				238.34		50.47732

				238.36		50.42893

				238.38		50.39374

				238.4		50.34974

				238.42		50.31015

				238.44		50.26176

				238.46		50.22216

				238.48		50.18697

				238.51		50.15178

				238.53		50.12098

				238.55		50.08139

				238.57		50.03739

				238.59		49.9978

				238.61		49.95381

				238.63		49.90981

				238.65		49.86582

				238.67		49.83943

				238.69		49.79103

				238.72		49.75584

				238.74		49.71185

				238.76		49.68545

				238.78		49.63266

				238.8		49.61066

				238.82		49.56667

				238.84		49.53148

				238.86		49.48748

				238.88		49.45229

				238.9		49.3995

				238.93		49.3599

				238.95		49.32031

				238.97		49.28072

				238.99		49.24552

				239.01		49.21033

				239.03		49.17074

				239.05		49.13114

				239.07		49.09155

				239.09		49.04756

				239.11		49.01236

				239.13		48.97717

				239.16		48.94197

				239.18		48.89798

				239.2		48.85399

				239.22		48.81439

				239.24		48.7792

				239.26		48.73521

				239.28		48.70001

				239.3		48.67362

				239.32		48.62962

				239.34		48.59443

				239.37		48.55924

				239.39		48.51964

				239.41		48.46685

				239.43		48.43166

				239.45		48.37887

				239.47		48.33487

				239.49		48.27768

				239.51		48.24689

				239.53		48.1985

				239.55		48.1545

				239.58		48.11491

				239.6		48.08851

				239.62		48.05332

				239.64		48.01373

				239.66		47.97853

				239.68		47.93894

				239.7		47.90814

				239.72		47.86415

				239.74		47.82896

				239.76		47.79376

				239.79		47.75417

				239.81		47.69698

				239.83		47.65738

				239.85		47.60899

				239.87		47.5694

				239.89		47.5386

				239.91		47.49461

				239.93		47.45062

				239.95		47.41542

				239.97		47.36703

				240		47.30984

				240.02		47.27905

				240.04		47.24385

				240.06		47.20866

				240.08		47.16906

				240.1		47.13387

				240.12		47.09868

				240.14		47.05468

				240.16		46.99749

				240.19		46.9711

				240.21		46.9359

				240.23		46.88751

				240.25		46.84352

				240.27		46.81712

				240.29		46.76433

				240.31		46.72914

				240.33		46.68074

				240.35		46.64115

				240.37		46.60596

				240.4		46.56196

				240.42		46.50917

				240.44		46.48278

				240.46		46.43878

				240.48		46.39479

				240.5		46.3508

				240.52		46.3508

				240.54		46.32

				240.56		46.28481

				240.58		46.22762

				240.61		46.18363

				240.63		46.10004

				240.65		46.03845

				240.67		45.98566

				240.69		45.95926

				240.71		45.92847

				240.73		45.89327

				240.75		45.84488

				240.77		45.80529

				240.79		45.7613

				240.82		45.7217

				240.84		45.68651

				240.86		45.64251

				240.88		45.61172

				240.9		45.57213

				240.92		45.53693

				240.94		45.48854

				240.96		45.45335

				240.98		45.40055

				241		45.34776

				241.03		45.30377

				241.05		45.26418

				241.07		45.22018

				241.09		45.17179

				241.11		45.1322

				241.13		45.08821

				241.15		45.04861

				241.17		45.00462

				241.19		44.97822

				241.21		44.95183

				241.24		44.90784

				241.26		44.86384

				241.28		44.82425

				241.3		44.77586

				241.32		44.72307

				241.34		44.67907

				241.36		44.63068

				241.38		44.59549

				241.4		44.54709

				241.42		44.4943

				241.45		44.44151

				241.47		44.40192

				241.49		44.34913

				241.51		44.30953

				241.53		44.26994

				241.55		44.23475

				241.57		44.19515

				241.59		44.15556

				241.61		44.11596

				241.63		44.09837

				241.66		44.06317

				241.68		44.03238

				241.7		43.99279

				241.72		43.94879

				241.74		43.8916

				241.76		43.84761

				241.78		43.79922

				241.8		43.75522

				241.82		43.70683

				241.84		43.66284

				241.87		43.61445

				241.89		43.57485

				241.91		43.53526

				241.93		43.48687

				241.95		43.44288

				241.97		43.41208

				241.99		43.36809

				242.01		43.3153

				242.03		43.2757

				242.05		43.23611

				242.08		43.18332

				242.1		43.13933

				242.12		43.09533

				242.14		43.06014

				242.16		43.01175

				242.18		42.96775

				242.2		42.91936

				242.22		42.88417

				242.24		42.84017

				242.26		42.79618

				242.29		42.74339

				242.31		42.71699

				242.33		42.6686

				242.35		42.62461

				242.37		42.58062

				242.39		42.55862

				242.41		42.49703

				242.43		42.44424

				242.45		42.39145

				242.47		42.34746

				242.5		42.29026

				242.52		42.24627

				242.54		42.20228

				242.56		42.16708

				242.58		42.11869

				242.6		42.0747

				242.62		42.02631

				242.64		41.99551

				242.66		41.95152

				242.68		41.89873

				242.71		41.86353

				242.73		41.82834

				242.75		41.77995

				242.77		41.73156

				242.79		41.69196

				242.81		41.64357

				242.83		41.59958

				242.85		41.54679

				242.87		41.49839

				242.89		41.4632

				242.92		41.41921

				242.94		41.36642

				242.96		41.32242

				242.98		41.28283

				243		41.23004

				243.02		41.18605

				243.04		41.15085

				243.06		41.11566

				243.08		41.06726

				243.11		41.02327

				243.13		40.96608

				243.15		40.93089

				243.17		40.8737

				243.19		40.8253

				243.21		40.78131

				243.23		40.75052

				243.25		40.69773

				243.27		40.65813

				243.29		40.61414

				243.32		40.58334

				243.34		40.53055

				243.36		40.48656

				243.38		40.45137

				243.4		40.41617

				243.42		40.35898

				243.44		40.31499

				243.46		40.2622

				243.48		40.2226

				243.5		40.16541

				243.53		40.12142

				243.55		40.07303

				243.57		40.03783

				243.59		39.98504

				243.61		39.94545

				243.63		39.90146

				243.65		39.86626

				243.67		39.81347

				243.69		39.75628

				243.71		39.71229

				243.74		39.6595

				243.76		39.6111

				243.78		39.57591

				243.8		39.53632

				243.82		39.50112

				243.84		39.46153

				243.86		39.40874

				243.88		39.35155

				243.9		39.32075

				243.92		39.25916

				243.95		39.21517

				243.97		39.17558

				243.99		39.13158

				244.01		39.07439

				244.03		39.0348

				244.05		38.97321

				244.07		38.92922

				244.09		38.88522

				244.11		38.83683

				244.13		38.77524

				244.16		38.77084

				244.18		38.71805

				244.2		38.67406

				244.22		38.63006

				244.24		38.59927

				244.26		38.52888

				244.28		38.48489

				244.3		38.4321

				244.32		38.3925

				244.34		38.34411

				244.37		38.29132

				244.39		38.24293

				244.41		38.20333

				244.43		38.14614

				244.45		38.11095

				244.47		38.07136

				244.49		38.03616

				244.51		37.97897

				244.53		37.93058

				244.55		37.87339

				244.58		37.8338

				244.6		37.781

				244.62		37.74141

				244.64		37.69742

				244.66		37.65782

				244.68		37.60503

				244.7		37.54784

				244.72		37.49505

				244.74		37.44666

				244.76		37.38507

				244.79		37.33668

				244.81		37.29268

				244.83		37.25749

				244.85		37.2091

				244.87		37.1651

				244.89		37.11231

				244.91		37.06832

				244.93		37.01993

				244.95		36.98034

				244.97		36.92754

				245		36.89675

				245.02		36.83956

				245.04		36.78677

				245.06		36.74277

				245.08		36.69878

				245.1		36.65479

				245.12		36.6108

				245.14		36.558

				245.16		36.50961

				245.18		36.46122

				245.21		36.40843

				245.23		36.36004

				245.25		36.30725

				245.27		36.25885

				245.29		36.21926

				245.31		36.17087

				245.33		36.13127

				245.35		36.09168

				245.37		36.03889

				245.39		35.9773

				245.42		35.92451

				245.44		35.87172

				245.46		35.82332

				245.48		35.77493

				245.5		35.73094

				245.52		35.69135

				245.54		35.64735

				245.56		35.59016

				245.58		35.55057

				245.61		35.49338

				245.63		35.45379

				245.65		35.40099

				245.67		35.357

				245.69		35.30421

				245.71		35.26462

				245.73		35.20303

				245.75		35.16343

				245.77		35.11944

				245.79		35.07105

				245.82		35.01386

				245.84		34.97426

				245.86		34.91267

				245.88		34.86868

				245.9		34.81589

				245.92		34.7807

				245.94		34.7279

				245.96		34.68831

				245.98		34.64872

				246		34.60033

				246.03		34.54753

				246.05		34.49914

				246.07		34.45075

				246.09		34.39356

				246.11		34.34517

				246.13		34.30117

				246.15		34.24398

				246.17		34.19999

				246.19		34.156

				246.21		34.11201

				246.24		34.05042

				246.26		34.01082

				246.28		33.95803

				246.3		33.90964

				246.32		33.85245

				246.34		33.82165

				246.36		33.77326

				246.38		33.72487

				246.4		33.67648

				246.42		33.62808

				246.45		33.57529

				246.47		33.5181

				246.49		33.47411

				246.51		33.42132

				246.53		33.37293

				246.55		33.32014

				246.57		33.26734

				246.59		33.21895

				246.61		33.17056

				246.63		33.11777

				246.66		33.07378

				246.68		33.02538

				246.7		32.96819

				246.72		32.9198

				246.74		32.87581

				246.76		32.82302

				246.78		32.77902

				246.8		32.73063

				246.82		32.67784

				246.84		32.63385

				246.87		32.58546

				246.89		32.52387

				246.91		32.47987

				246.93		32.43588

				246.95		32.38309

				246.97		32.3303

				246.99		32.28631

				247.01		32.24671

				247.03		32.19392

				247.05		32.14553

				247.08		32.10593

				247.1		32.05754

				247.12		32.00035

				247.14		31.94756

				247.16		31.90357

				247.18		31.85078

				247.2		31.79799

				247.22		31.74079

				247.24		31.7012

				247.26		31.63521

				247.29		31.58682

				247.31		31.52083

				247.33		31.47244

				247.35		31.41085

				247.37		31.37565

				247.39		31.32286

				247.41		31.28767

				247.43		31.23488

				247.45		31.18649

				247.47		31.13369

				247.5		31.0853

				247.52		31.03251

				247.54		30.98412

				247.56		30.94013

				247.58		30.88294

				247.6		30.83454

				247.62		30.78615

				247.64		30.72896

				247.66		30.67617

				247.68		30.62338

				247.71		30.56619

				247.73		30.5178

				247.75		30.4694

				247.77		30.41661

				247.79		30.37262

				247.81		30.31983

				247.83		30.26704

				247.85		30.22744

				247.87		30.17465

				247.89		30.12186

				247.92		30.07787

				247.94		30.02948

				247.96		29.96789

				247.98		29.91949

				248		29.8711

				248.02		29.82271

				248.04		29.76992

				248.06		29.73912

				248.08		29.69073

				248.11		29.63794

				248.13		29.58955

				248.15		29.53236

				248.17		29.46637

				248.19		29.40478

				248.21		29.35639

				248.23		29.29919

				248.25		29.2464

				248.27		29.19801

				248.29		29.15842

				248.32		29.10123

				248.34		29.04844

				248.36		29.00444

				248.38		28.95605

				248.4		28.90326

				248.42		28.85927

				248.44		28.80648

				248.46		28.74929

				248.48		28.69649

				248.5		28.6437

				248.53		28.59091

				248.55		28.54692

				248.57		28.48973

				248.59		28.43694

				248.61		28.38854

				248.63		28.33135

				248.65		28.29176

				248.67		28.24777

				248.69		28.19938

				248.71		28.13779

				248.74		28.08939

				248.76		28.0278

				248.78		27.97941

				248.8		27.92662

				248.82		27.87823

				248.84		27.82984

				248.86		27.77265

				248.88		27.71985

				248.9		27.65826

				248.92		27.60987

				248.95		27.55708

				248.97		27.51309

				248.99		27.4559

				249.01		27.4163

				249.03		27.36791

				249.05		27.31072

				249.07		27.25353

				249.09		27.19194

				249.11		27.13915

				249.13		27.08196

				249.16		27.02917

				249.18		26.98517

				249.2		26.93678

				249.22		26.87959

				249.24		26.8312

				249.26		26.78281

				249.28		26.73442

				249.3		26.69042

				249.32		26.63323

				249.34		26.58924

				249.37		26.53205

				249.39		26.47046

				249.41		26.40447

				249.43		26.35608

				249.45		26.29449

				249.47		26.25049

				249.49		26.1933

				249.51		26.14491

				249.53		26.09652

				249.55		26.03933

				249.58		25.97774

				249.6		25.92935

				249.62		25.87216

				249.64		25.81937

				249.66		25.76657

				249.68		25.71818

				249.7		25.66099

				249.72		25.617

				249.74		25.55541

				249.77		25.50702

				249.79		25.46302

				249.81		25.41903

				249.83		25.35744

				249.85		25.31345

				249.87		25.26066

				249.89		25.19907

				249.91		25.13748

				249.93		25.09348

				249.95		25.03629

				249.98		24.9835

				250		24.92191

				250.02		24.87352

				250.04		24.81193

				250.06		24.76354

				250.08		24.71515

				250.1		24.66675

				250.12		24.61396

				250.14		24.56997

				250.16		24.50838

				250.19		24.45999

				250.21		24.4072

				250.23		24.35441

				250.25		24.29282

				250.27		24.24442

				250.29		24.18723

				250.31		24.13004

				250.33		24.06845

				250.35		24.02006

				250.37		23.96287

				250.4		23.91008

				250.42		23.84849

				250.44		23.8089

				250.46		23.7517

				250.48		23.69891

				250.5		23.64612

				250.52		23.59773

				250.54		23.53614

				250.56		23.48775

				250.58		23.42176

				250.61		23.37337

				250.63		23.32497

				250.65		23.26778

				250.67		23.20179

				250.69		23.1622

				250.71		23.09621

				250.73		23.04342

				250.75		22.98623

				250.77		22.94664

				250.79		22.89385

				250.82		22.84545

				250.84		22.79266

				250.86		22.75307

				250.88		22.70028

				250.9		22.63869

				250.92		22.5859

				250.94		22.5419

				250.96		22.48471

				250.98		22.42752

				251		22.36593

				251.03		22.32194

				251.05		22.26475

				251.07		22.20756

				251.09		22.15477

				251.11		22.11077

				251.13		22.04918

				251.15		22.00079

				251.17		21.9392

				251.19		21.88641

				251.21		21.83362

				251.24		21.78083

				251.26		21.71484

				251.28		21.67964

				251.3		21.62245

				251.32		21.55646

				251.34		21.49487

				251.36		21.44208

				251.38		21.38049

				251.4		21.3189

				251.42		21.27051

				251.45		21.23092

				251.47		21.17813

				251.49		21.11214

				251.51		21.06375

				251.53		21.01095

				251.55		20.94497

				251.57		20.88777

				251.59		20.83938

				251.61		20.78659

				251.63		20.725

				251.66		20.67221

				251.68		20.61502

				251.7		20.55783

				251.72		20.50504

				251.74		20.44345

				251.76		20.38186

				251.78		20.32467

				251.8		20.27188

				251.82		20.21908

				251.84		20.16629

				251.87		20.1179

				251.89		20.06951

				251.91		20.01232

				251.93		19.95513

				251.95		19.90674

				251.97		19.84954

				251.99		19.79235

				252.01		19.73956

				252.03		19.67797

				252.05		19.62518

				252.08		19.57679

				252.1		19.524

				252.12		19.47121

				252.14		19.42281

				252.16		19.36122

				252.18		19.29524

				252.2		19.24244

				252.22		19.18085

				252.24		19.12806

				252.26		19.07087

				252.29		19.02688

				252.31		18.96529

				252.33		18.9125

				252.35		18.85531

				252.37		18.81131

				252.39		18.74973

				252.41		18.69693

				252.43		18.63534

				252.45		18.59135

				252.47		18.53856

				252.5		18.49017

				252.52		18.42418

				252.54		18.38019

				252.56		18.3142

				252.58		18.25261

				252.6		18.20421

				252.62		18.15582

				252.64		18.10303

				252.66		18.05024

				252.68		17.99745

				252.71		17.94026

				252.73		17.88747

				252.75		17.81708

				252.77		17.75989

				252.79		17.7115

				252.81		17.64991

				252.83		17.58832

				252.85		17.54872

				252.87		17.49153

				252.89		17.43434

				252.91		17.38155

				252.94		17.33316

				252.96		17.28477

				252.98		17.22318

				253		17.16159

				253.02		17.10439

				253.04		17.0516

				253.06		16.99001

				253.08		16.92842

				253.1		16.88003

				253.12		16.82724

				253.15		16.77005

				253.17		16.69966

				253.19		16.64687

				253.21		16.58968

				253.23		16.52369

				253.25		16.4665

				253.27		16.42251

				253.29		16.37411

				253.31		16.32572

				253.33		16.26853

				253.36		16.22454

				253.38		16.16735

				253.4		16.10136

				253.42		16.03977

				253.44		15.99578

				253.46		15.93419

				253.48		15.877

				253.5		15.8242

				253.52		15.77581

				253.54		15.71862

				253.57		15.66143

				253.59		15.61304

				253.61		15.56465

				253.63		15.51186

				253.65		15.45027

				253.67		15.40187

				253.69		15.34468

				253.71		15.28749

				253.73		15.2303

				253.75		15.17311

				253.78		15.11152

				253.8		15.05873

				253.82		15.00594

				253.84		14.94875

				253.86		14.90036

				253.88		14.84756

				253.9		14.79037

				253.92		14.72878

				253.94		14.67599

				253.96		14.6276

				253.99		14.57481

				254.01		14.51762

				254.03		14.46043

				254.05		14.41644

				254.07		14.35485

				254.09		14.29766

				254.11		14.25366

				254.13		14.20087

				254.15		14.14808

				254.17		14.08649

				254.2		14.0337

				254.22		13.97651

				254.24		13.92372

				254.26		13.85773

				254.28		13.80934

				254.3		13.75214

				254.32		13.69935

				254.34		13.63776

				254.36		13.58497

				254.38		13.52778

				254.41		13.45739

				254.43		13.3958

				254.45		13.33861

				254.47		13.29902

				254.49		13.23743

				254.51		13.19344

				254.53		13.14064

				254.55		13.09665

				254.57		13.03506

				254.59		12.98227

				254.62		12.92948

				254.64		12.87229

				254.66		12.8107

				254.68		12.74911

				254.7		12.70512

				254.72		12.63913

				254.74		12.59074

				254.76		12.53354

				254.78		12.48955

				254.8		12.43236

				254.82		12.38837

				254.85		12.31798

				254.87		12.28279

				254.89		12.2124

				254.91		12.15081

				254.93		12.08922

				254.95		12.04083

				254.97		11.97484

				254.99		11.93084

				255.01		11.86925

				255.03		11.82526

				255.06		11.76807

				255.08		11.71528

				255.1		11.66249

				255.12		11.62289

				255.14		11.5569

				255.16		11.50851

				255.18		11.45572

				255.2		11.39413

				255.22		11.33254

				255.24		11.28415

				255.27		11.21376

				255.29		11.15217

				255.31		11.09938

				255.33		11.03779

				255.35		10.9894

				255.37		10.9542

				255.39		10.90581

				255.41		10.85302

				255.43		10.79583

				255.45		10.73864

				255.47		10.68585

				255.5		10.62866

				255.52		10.57587

				255.54		10.52747

				255.56		10.47468

				255.58		10.41309

				255.6		10.3647

				255.62		10.31631

				255.64		10.26792

				255.66		10.21512

				255.68		10.15793

				255.71		10.10514

				255.73		10.04355

				255.75		9.981963

				255.77		9.915974

				255.79		9.867582

				255.81		9.805992

				255.83		9.7576

				255.85		9.69601

				255.87		9.647618

				255.89		9.599226

				255.92		9.546434

				255.94		9.493643

				255.96		9.44965

				255.98		9.405657

				256		9.348467

				256.02		9.295676

				256.04		9.234086

				256.06		9.176895

				256.08		9.115305

				256.1		9.066913

				256.12		9.009722

				256.15		8.96133

				256.17		8.908539

				256.19		8.860147

				256.21		8.807356

				256.23		8.767762

				256.25		8.71937

				256.27		8.662179

				256.29		8.609388

				256.31		8.560996

				256.33		8.503805

				256.36		8.437816

				256.38		8.398223

				256.4		8.345431

				256.42		8.288241

				256.44		8.226651

				256.46		8.178259

				256.48		8.129867

				256.5		8.077075

				256.52		8.028683

				256.54		7.971493

				256.56		7.9275

				256.59		7.861511

				256.61		7.813119

				256.63		7.755928

				256.65		7.711935

				256.67		7.663543

				256.69		7.610752

				256.71		7.553561

				256.73		7.522766

				256.75		7.461176

				256.77		7.399586

				256.8		7.346795

				256.82		7.302802

				256.84		7.241212

				256.86		7.188421

				256.88		7.144428

				256.9		7.109234

				256.92		7.056443

				256.94		6.994853

				256.96		6.946461

				256.98		6.898069

				257		6.836479

				257.03		6.788087

				257.05		6.748493

				257.07		6.713299

				257.09		6.660508

				257.11		6.607716

				257.13		6.554925

				257.15		6.515331

				257.17		6.453742

				257.19		6.40095

				257.21		6.352558

				257.24		6.308565

				257.26		6.251375

				257.28		6.202983

				257.3		6.154591

				257.32		6.119396

				257.34		6.071004

				257.36		6.013814

				257.38		5.969821

				257.4		5.925828

				257.42		5.873037

				257.45		5.824645

				257.47		5.785051

				257.49		5.741058

				257.51		5.692666

				257.53		5.639875

				257.55		5.595882

				257.57		5.551889

				257.59		5.503497

				257.61		5.459505

				257.63		5.406713

				257.66		5.358321

				257.68		5.30553

				257.7		5.257138

				257.72		5.204346

				257.74		5.186749

				257.76		5.138357

				257.78		5.089965

				257.8		5.054771

				257.82		5.019577

				257.84		4.957987

				257.86		4.918393

				257.89		4.874401

				257.91		4.830408

				257.93		4.782016

				257.95		4.738023

				257.97		4.702829

				257.99		4.676433

				258.01		4.63244

				258.03		4.588447

				258.05		4.553253

				258.07		4.491663

				258.1		4.443271

				258.12		4.399279

				258.14		4.364084

				258.16		4.333289

				258.18		4.306894

				258.2		4.262901

				258.22		4.223307

				258.24		4.183714

				258.26		4.135322

				258.28		4.095728

				258.3		4.064933

				258.33		4.034138

				258.35		4.003343

				258.37		3.96375

				258.39		3.937354

				258.41		3.897761

				258.43		3.862567

				258.45		3.827372

				258.47		3.800977

				258.49		3.765782

				258.51		3.743786

				258.54		3.71739

				258.56		3.690995

				258.58		3.673398

				258.6		3.651401

				258.62		3.625005

				258.64		3.59861

				258.66		3.572214

				258.68		3.541419

				258.7		3.506225

				258.72		3.484229

				258.74		3.462232

				258.77		3.440236

				258.79		3.41384

				258.81		3.405042

				258.83		3.383045

				258.85		3.361049

				258.87		3.343452

				258.89		3.334653

				258.91		3.317056

				258.93		3.29066

				258.95		3.273063

				258.97		3.251067

				259		3.23347

				259.02		3.215873

				259.04		3.202675

				259.06		3.202675

				259.08		3.189477

				259.1		3.17188

				259.12		3.17188

				259.14		3.158682

				259.16		3.141085

				259.18		3.127887

				259.21		3.123488

				259.23		3.092693

				259.25		3.092693

				259.27		3.075096

				259.29		3.061898

				259.31		3.0487

				259.33		3.053099

				259.35		3.039901

				259.37		3.039901

				259.39		3.035502

				259.41		3.039901

				259.44		3.035502

				259.46		3.017905

				259.48		3.013506

				259.5		3.004707

				259.52		3.000308

				259.54		2.978312

				259.56		2.969513

				259.58		2.965114

				259.6		2.960714

				259.62		2.951916

				259.64		2.951916

				259.67		2.947517

				259.69		2.943117

				259.71		2.938718

				259.73		2.934319

				259.75		2.938718

				259.77		2.943117

				259.79		2.938718

				259.81		2.934319

				259.83		2.934319

				259.85		2.934319

				259.87		2.934319

				259.9		2.934319

				259.92		2.934319

				259.94		2.934319

				259.96		2.929919

				259.98		2.92552

				260		2.921121

				260.02		2.916722

				260.04		2.916722

				260.06		2.916722

				260.08		2.912322

				260.1		2.912322

				260.13		2.907923

				260.15		2.903524

				260.17		2.894725

				260.19		2.890326

				260.21		2.885927

				260.23		2.885927

				260.25		2.881527

				260.27		2.877128

				260.29		2.877128

				260.31		2.877128

				260.33		2.872729

				260.36		2.86833

				260.38		2.86833

				260.4		2.86393

				260.42		2.86393

				260.44		2.859531

				260.46		2.855132

				260.48		2.855132

				260.5		2.850732

				260.52		2.850732

				260.54		2.846333

				260.56		2.850732

				260.59		2.846333

				260.61		2.846333

				260.63		2.841934

				260.65		2.841934

				260.67		2.837535

				260.69		2.837535

				260.71		2.833135

				260.73		2.833135

				260.75		2.833135

				260.77		2.828736

				260.79		2.828736

				260.81		2.828736

				260.84		2.828736

				260.86		2.824337

				260.88		2.824337

				260.9		2.824337

				260.92		2.819938

				260.94		2.819938

				260.96		2.819938

				260.98		2.815538

				261		2.815538

				261.02		2.815538

				261.04		2.815538

				261.07		2.811139

				261.09		2.811139

				261.11		2.811139

				261.13		2.811139

				261.15		2.811139

				261.17		2.811139

				261.19		2.80674

				261.21		2.80674

				261.23		2.80674

				261.25		2.80674

				261.27		2.80234

				261.3		2.80234

				261.32		2.80234

				261.34		2.80234

				261.36		2.797941

				261.38		2.797941

				261.4		2.797941

				261.42		2.793542

				261.44		2.793542

				261.46		2.793542

				261.48		2.793542

				261.5		2.793542

				261.53		2.793542

				261.55		2.793542

				261.57		2.793542

				261.59		2.789143

				261.61		2.789143

				261.63		2.789143

				261.65		2.789143

				261.67		2.789143

				261.69		2.789143

				261.71		2.784743

				261.73		2.784743

				261.76		2.784743

				261.78		2.784743

				261.8		2.784743

				261.82		2.780344

				261.84		2.780344

				261.86		2.780344

				261.88		2.780344

				261.9		2.780344

				261.92		2.780344

				261.94		2.775945

				261.96		2.775945

				261.98		2.775945

				262.01		2.775945

				262.03		2.775945

				262.05		2.775945

				262.07		2.775945

				262.09		2.775945

				262.11		2.775945

				262.13		2.775945

				262.15		2.775945

				262.17		2.771545

				262.19		2.771545

				262.21		2.771545

				262.24		2.771545

				262.26		2.771545

				262.28		2.771545

				262.3		2.771545

				262.32		2.771545

				262.34		2.767146

				262.36		2.767146

				262.38		2.767146

				262.4		2.767146

				262.42		2.767146

				262.44		2.767146

				262.46		2.767146

				262.49		2.767146

				262.51		2.767146

				262.53		2.762747

				262.55		2.762747

				262.57		2.762747

				262.59		2.762747

				262.61		2.762747

				262.63		2.762747

				262.65		2.758348

				262.67		2.758348

				262.69		2.758348

				262.72		2.758348

				262.74		2.758348

				262.76		2.753948

				262.78		2.753948

				262.8		2.753948

				262.82		2.753948

				262.84		2.753948

				262.86		2.753948

				262.88		2.753948

				262.9		2.753948

				262.92		2.753948

				262.95		2.753948

				262.97		2.749549

				262.99		2.749549

				263.01		2.749549

				263.03		2.749549

				263.05		2.749549

				263.07		2.749549

				263.09		2.749549

				263.11		2.749549

				263.13		2.749549

				263.15		2.74515

				263.17		2.74515

				263.2		2.74515

				263.22		2.74515

				263.24		2.74515

				263.26		2.74515

				263.28		2.74515

				263.3		2.74515

				263.32		2.740751

				263.34		2.740751

				263.36		2.740751

				263.38		2.740751

				263.4		2.740751

				263.42		2.740751

				263.45		2.740751

				263.47		2.736351

				263.49		2.736351

				263.51		2.736351

				263.53		2.736351

				263.55		2.736351

				263.57		2.731952

				263.59		2.731952

				263.61		2.731952

				263.63		2.731952

				263.65		2.731952

				263.68		2.727553

				263.7		2.727553

				263.72		2.727553

				263.74		2.727553

				263.76		2.727553

				263.78		2.727553

				263.8		2.723153

				263.82		2.723153

				263.84		2.723153

				263.86		2.718754

				263.88		2.718754

				263.9		2.718754

				263.93		2.718754

				263.95		2.718754

				263.97		2.718754

				263.99		2.718754

				264.01		2.714355

				264.03		2.714355

				264.05		2.714355

				264.07		2.714355

				264.09		2.714355

				264.11		2.714355

				264.13		2.714355

				264.15		2.714355

				264.18		2.714355

				264.2		2.709956

				264.22		2.709956

				264.24		2.709956

				264.26		2.709956

				264.28		2.709956

				264.3		2.709956

				264.32		2.709956

				264.34		2.709956

				264.36		2.709956

				264.38		2.705556

				264.4		2.705556

				264.43		2.705556

				264.45		2.705556

				264.47		2.705556

				264.49		2.705556

				264.51		2.705556

				264.53		2.701157

				264.55		2.701157

				264.57		2.701157

				264.59		2.701157

				264.61		2.701157

				264.63		2.701157

				264.66		2.701157

				264.68		2.701157

				264.7		2.701157

				264.72		2.696758

				264.74		2.696758

				264.76		2.696758

				264.78		2.696758

				264.8		2.696758

				264.82		2.696758

				264.84		2.696758

				264.86		2.696758

				264.88		2.696758

				264.91		2.692358

				264.93		2.692358

				264.95		2.692358

				264.97		2.692358

				264.99		2.692358

				265.01		2.692358

				265.03		2.692358

				265.05		2.687959

				265.07		2.687959

				265.09		2.687959

				265.11		2.687959

				265.14		2.687959

				265.16		2.687959

				265.18		2.687959

				265.2		2.68356

				265.22		2.68356

				265.24		2.68356

				265.26		2.68356

				265.28		2.68356

				265.3		2.679161

				265.32		2.679161

				265.34		2.679161

				265.36		2.679161

				265.39		2.679161

				265.41		2.679161

				265.43		2.679161

				265.45		2.679161

				265.47		2.679161

				265.49		2.679161

				265.51		2.674761

				265.53		2.674761

				265.55		2.674761

				265.57		2.674761

				265.59		2.674761

				265.62		2.674761

				265.64		2.674761

				265.66		2.674761

				265.68		2.674761

				265.7		2.670362

				265.72		2.670362

				265.74		2.670362

				265.76		2.670362

				265.78		2.670362

				265.8		2.670362

				265.82		2.670362

				265.84		2.670362

				265.87		2.670362

				265.89		2.670362

				265.91		2.670362

				265.93		2.665963

				265.95		2.665963

				265.97		2.665963

				265.99		2.665963

				266.01		2.665963

				266.03		2.665963

				266.05		2.665963

				266.07		2.665963

				266.1		2.665963

				266.12		2.665963

				266.14		2.665963

				266.16		2.665963

				266.18		2.665963

				266.2		2.661564

				266.22		2.661564

				266.24		2.661564

				266.26		2.661564

				266.28		2.661564

				266.3		2.661564

				266.32		2.661564

				266.35		2.661564

				266.37		2.661564

				266.39		2.661564

				266.41		2.657164

				266.43		2.657164

				266.45		2.657164

				266.47		2.657164

				266.49		2.657164

				266.51		2.657164

				266.53		2.657164

				266.55		2.657164

				266.58		2.657164

				266.6		2.657164

				266.62		2.657164

				266.64		2.652765

				266.66		2.652765

				266.68		2.652765

				266.7		2.652765

				266.72		2.652765

				266.74		2.652765

				266.76		2.652765

				266.78		2.652765

				266.8		2.652765

				266.83		2.652765

				266.85		2.648366

				266.87		2.648366

				266.89		2.648366

				266.91		2.648366

				266.93		2.648366

				266.95		2.648366

				266.97		2.648366

				266.99		2.648366

				267.01		2.648366

				267.03		2.648366

				267.05		2.648366

				267.08		2.648366

				267.1		2.643966

				267.12		2.643966

				267.14		2.643966

				267.16		2.643966

				267.18		2.643966

				267.2		2.643966

				267.22		2.643966

				267.24		2.643966

				267.26		2.643966

				267.28		2.643966

				267.3		2.643966

				267.33		2.643966

				267.35		2.643966

				267.37		2.643966

				267.39		2.643966

				267.41		2.643966

				267.43		2.643966

				267.45		2.643966

				267.47		2.643966

				267.49		2.643966

				267.51		2.643966

				267.53		2.643966

				267.55		2.643966

				267.58		2.639567

				267.6		2.639567

				267.62		2.639567

				267.64		2.639567

				267.66		2.639567

				267.68		2.639567

				267.7		2.639567

				267.72		2.639567

				267.74		2.639567

				267.76		2.639567

				267.78		2.639567

				267.8		2.639567

				267.83		2.639567

				267.85		2.639567

				267.87		2.635168

				267.89		2.635168

				267.91		2.635168

				267.93		2.635168

				267.95		2.635168

				267.97		2.635168

				267.99		2.635168

				268.01		2.635168

				268.03		2.635168

				268.05		2.635168

				268.08		2.635168

				268.1		2.635168

				268.12		2.635168

				268.14		2.630769

				268.16		2.630769

				268.18		2.630769

				268.2		2.630769

				268.22		2.630769

				268.24		2.630769

				268.26		2.630769

				268.28		2.630769

				268.3		2.630769

				268.33		2.630769

				268.35		2.630769

				268.37		2.630769

				268.39		2.630769

				268.41		2.630769

				268.43		2.626369

				268.45		2.626369

				268.47		2.626369

				268.49		2.626369

				268.51		2.626369

				268.53		2.626369

				268.55		2.626369

				268.57		2.626369

				268.6		2.626369

				268.62		2.626369

				268.64		2.626369

				268.66		2.626369

				268.68		2.626369

				268.7		2.62197

				268.72		2.62197

				268.74		2.62197

				268.76		2.62197

				268.78		2.62197

				268.8		2.62197

				268.82		2.62197

				268.85		2.62197

				268.87		2.62197

				268.89		2.62197

				268.91		2.62197

				268.93		2.62197

				268.95		2.62197

				268.97		2.62197

				268.99		2.62197

				269.01		2.617571

				269.03		2.617571

				269.05		2.617571

				269.07		2.617571

				269.1		2.617571

				269.12		2.617571

				269.14		2.617571

				269.16		2.617571

				269.18		2.617571

				269.2		2.617571

				269.22		2.617571

				269.24		2.617571

				269.26		2.617571

				269.28		2.613171

				269.3		2.613171

				269.32		2.613171

				269.34		2.613171

				269.37		2.613171

				269.39		2.613171

				269.41		2.613171

				269.43		2.613171

				269.45		2.613171

				269.47		2.613171

				269.49		2.608772

				269.51		2.608772

				269.53		2.608772

				269.55		2.608772

				269.57		2.608772

				269.59		2.608772

				269.62		2.608772

				269.64		2.608772

				269.66		2.604373

				269.68		2.604373

				269.7		2.604373

				269.72		2.604373

				269.74		2.604373

				269.76		2.604373

				269.78		2.604373

				269.8		2.599974

				269.82		2.604373

				269.84		2.599974

				269.87		2.599974

				269.89		2.599974

				269.91		2.599974

				269.93		2.599974

				269.95		2.599974

				269.97		2.599974

				269.99		2.599974

				270.01		2.595574

				270.03		2.595574

				270.05		2.595574

				270.07		2.595574

				270.09		2.595574

				270.12		2.595574

				270.14		2.595574

				270.16		2.595574

				270.18		2.595574

				270.2		2.595574

				270.22		2.595574

				270.24		2.595574

				270.26		2.595574

				270.28		2.591175

				270.3		2.591175

				270.32		2.591175

				270.34		2.591175

				270.37		2.591175

				270.39		2.591175

				270.41		2.591175

				270.43		2.591175

				270.45		2.586776

				270.47		2.586776

				270.49		2.586776

				270.51		2.586776

				270.53		2.586776

				270.55		2.586776

				270.57		2.586776

				270.59		2.586776

				270.62		2.586776

				270.64		2.582376

				270.66		2.582376

				270.68		2.582376

				270.7		2.582376

				270.72		2.582376

				270.74		2.582376

				270.76		2.582376

				270.78		2.582376

				270.8		2.582376

				270.82		2.582376

				270.85		2.577977

				270.87		2.577977

				270.89		2.577977

				270.91		2.577977

				270.93		2.577977

				270.95		2.577977

				270.97		2.577977

				270.99		2.577977

				271.01		2.577977

				271.03		2.577977

				271.05		2.573578

				271.07		2.573578

				271.1		2.573578

				271.12		2.573578

				271.14		2.573578

				271.16		2.573578

				271.18		2.573578

				271.2		2.573578

				271.22		2.569179

				271.24		2.569179

				271.26		2.569179

				271.28		2.569179

				271.3		2.569179

				271.33		2.569179

				271.35		2.569179

				271.37		2.569179

				271.39		2.564779

				271.41		2.564779

				271.43		2.564779

				271.45		2.564779

				271.47		2.564779

				271.49		2.564779

				271.51		2.564779

				271.53		2.564779

				271.55		2.564779

				271.58		2.564779

				271.6		2.564779

				271.62		2.564779

				271.64		2.564779

				271.66		2.564779

				271.68		2.564779

				271.7		2.56038

				271.72		2.56038

				271.74		2.56038

				271.76		2.56038

				271.78		2.56038

				271.81		2.56038

				271.83		2.56038

				271.85		2.56038

				271.87		2.56038

				271.89		2.56038

				271.91		2.56038

				271.93		2.56038

				271.95		2.555981

				271.97		2.555981

				271.99		2.555981

				272.01		2.555981

				272.04		2.555981

				272.06		2.555981

				272.08		2.555981

				272.1		2.555981

				272.12		2.555981

				272.14		2.555981

				272.16		2.555981

				272.18		2.555981

				272.2		2.551582

				272.22		2.551582

				272.24		2.551582

				272.27		2.551582

				272.29		2.551582

				272.31		2.551582

				272.33		2.551582

				272.35		2.551582

				272.37		2.551582

				272.39		2.547182

				272.41		2.547182

				272.43		2.547182

				272.45		2.547182

				272.47		2.547182

				272.5		2.547182

				272.52		2.547182

				272.54		2.547182

				272.56		2.547182

				272.58		2.547182

				272.6		2.547182

				272.62		2.547182

				272.64		2.547182

				272.66		2.547182

				272.68		2.547182

				272.7		2.547182

				272.73		2.547182

				272.75		2.547182

				272.77		2.547182

				272.79		2.547182

				272.81		2.547182

				272.83		2.547182

				272.85		2.547182

				272.87		2.542783

				272.89		2.542783

				272.91		2.542783

				272.93		2.542783

				272.95		2.542783

				272.98		2.542783

				273		2.542783

				273.02		2.542783

				273.04		2.542783

				273.06		2.542783

				273.08		2.542783

				273.1		2.542783

				273.12		2.542783

				273.14		2.542783

				273.16		2.542783

				273.18		2.542783

				273.21		2.542783

				273.23		2.542783

				273.25		2.538384

				273.27		2.538384

				273.29		2.538384

				273.31		2.538384

				273.33		2.538384

				273.35		2.538384

				273.37		2.538384

				273.39		2.538384

				273.41		2.538384

				273.43		2.538384

				273.46		2.538384

				273.48		2.538384

				273.5		2.538384

				273.52		2.538384

				273.54		2.538384

				273.56		2.538384

				273.58		2.533984

				273.6		2.533984

				273.62		2.533984

				273.64		2.533984

				273.66		2.533984

				273.69		2.533984

				273.71		2.533984

				273.73		2.533984

				273.75		2.533984

				273.77		2.529585

				273.79		2.529585

				273.81		2.529585

				273.83		2.529585

				273.85		2.529585

				273.87		2.529585

				273.89		2.529585

				273.91		2.529585

				273.94		2.529585

				273.96		2.529585

				273.98		2.529585

				274		2.529585

				274.02		2.529585

				274.04		2.529585

				274.06		2.529585

				274.08		2.529585

				274.1		2.529585

				274.12		2.529585

				274.14		2.525186

				274.17		2.525186

				274.19		2.525186

				274.21		2.525186

				274.23		2.525186

				274.25		2.525186

				274.27		2.525186

				274.29		2.525186

				274.31		2.525186

				274.33		2.525186

				274.35		2.520787

				274.37		2.520787

				274.4		2.520787

				274.42		2.520787

				274.44		2.520787

				274.46		2.520787

				274.48		2.520787

				274.5		2.520787

				274.52		2.520787

				274.54		2.520787

				274.56		2.520787

				274.58		2.516387

				274.6		2.516387

				274.62		2.516387

				274.65		2.516387

				274.67		2.516387

				274.69		2.516387

				274.71		2.516387

				274.73		2.511988

				274.75		2.511988

				274.77		2.511988

				274.79		2.511988

				274.81		2.511988

				274.83		2.511988

				274.85		2.511988

				274.88		2.507589

				274.9		2.507589

				274.92		2.507589

				274.94		2.507589

				274.96		2.507589

				274.98		2.507589

				275		2.507589

				275.02		2.507589

				275.04		2.503189

				275.06		2.503189

				275.08		2.503189

				275.11		2.503189

				275.13		2.503189

				275.15		2.503189

				275.17		2.503189

				275.19		2.503189

				275.21		2.503189

				275.23		2.49879

				275.25		2.49879

				275.27		2.49879

				275.29		2.49879

				275.31		2.49879

				275.33		2.49879

				275.36		2.49879

				275.38		2.49879

				275.4		2.49879

				275.42		2.49879

				275.44		2.49879

				275.46		2.49879

				275.48		2.49879

				275.5		2.494391

				275.52		2.494391

				275.54		2.494391

				275.56		2.494391

				275.59		2.494391

				275.61		2.494391

				275.63		2.494391

				275.65		2.494391

				275.67		2.494391

				275.69		2.494391

				275.71		2.489992

				275.73		2.489992

				275.75		2.489992

				275.77		2.489992

				275.79		2.489992

				275.82		2.489992

				275.84		2.489992

				275.86		2.489992

				275.88		2.489992

				275.9		2.489992

				275.92		2.485592

				275.94		2.485592

				275.96		2.485592

				275.98		2.485592

				276		2.485592

				276.02		2.485592

				276.05		2.485592

				276.07		2.485592

				276.09		2.485592

				276.11		2.485592

				276.13		2.481193

				276.15		2.481193

				276.17		2.481193

				276.19		2.481193

				276.21		2.481193

				276.23		2.481193

				276.25		2.481193

				276.28		2.481193

				276.3		2.481193

				276.32		2.481193

				276.34		2.481193

				276.36		2.481193

				276.38		2.481193

				276.4		2.481193

				276.42		2.481193

				276.44		2.481193

				276.46		2.481193

				276.48		2.481193

				276.51		2.481193

				276.53		2.481193

				276.55		2.481193

				276.57		2.481193

				276.59		2.481193

				276.61		2.481193

				276.63		2.481193

				276.65		2.481193

				276.67		2.481193

				276.69		2.481193

				276.71		2.476794

				276.74		2.481193

				276.76		2.476794

				276.78		2.481193

				276.8		2.476794

				276.82		2.476794

				276.84		2.476794

				276.86		2.476794

				276.88		2.476794

				276.9		2.476794

				276.92		2.476794

				276.95		2.476794

				276.97		2.476794

				276.99		2.476794

				277.01		2.476794

				277.03		2.476794

				277.05		2.476794

				277.07		2.476794

				277.09		2.476794

				277.11		2.476794

				277.13		2.476794

				277.15		2.476794

				277.18		2.476794

				277.2		2.476794

				277.22		2.476794

				277.24		2.476794

				277.26		2.476794

				277.28		2.476794

				277.3		2.476794

				277.32		2.476794

				277.34		2.476794

				277.36		2.472395

				277.39		2.472395

				277.41		2.472395

				277.43		2.472395

				277.45		2.472395

				277.47		2.472395

				277.49		2.476794

				277.51		2.476794

				277.53		2.472395

				277.55		2.472395

				277.57		2.472395

				277.59		2.472395

				277.62		2.472395

				277.64		2.472395

				277.66		2.472395

				277.68		2.472395

				277.7		2.472395

				277.72		2.472395

				277.74		2.472395

				277.76		2.472395

				277.78		2.472395

				277.8		2.472395

				277.82		2.472395

				277.85		2.472395

				277.87		2.472395

				277.89		2.472395

				277.91		2.472395

				277.93		2.472395

				277.95		2.472395

				277.97		2.472395

				277.99		2.472395

				278.01		2.472395

				278.03		2.472395

				278.06		2.472395

				278.08		2.472395

				278.1		2.472395

				278.12		2.472395

				278.14		2.472395

				278.16		2.472395

				278.18		2.472395

				278.2		2.472395

				278.22		2.467995

				278.24		2.467995

				278.26		2.467995

				278.29		2.467995

				278.31		2.467995

				278.33		2.467995

				278.35		2.467995

				278.37		2.467995

				278.39		2.467995

				278.41		2.467995

				278.43		2.467995

				278.45		2.463596

				278.47		2.463596

				278.49		2.463596

				278.52		2.463596

				278.54		2.463596

				278.56		2.463596

				278.58		2.463596

				278.6		2.463596

				278.62		2.463596

				278.64		2.463596

				278.66		2.463596

				278.68		2.463596

				278.7		2.463596

				278.72		2.463596

				278.75		2.463596

				278.77		2.459197

				278.79		2.459197

				278.81		2.459197

				278.83		2.459197

				278.85		2.459197

				278.87		2.459197

				278.89		2.459197

				278.91		2.459197

				278.93		2.459197

				278.95		2.459197

				278.98		2.459197

				279		2.459197

				279.02		2.459197

				279.04		2.459197

				279.06		2.459197

				279.08		2.459197

				279.1		2.459197

				279.12		2.459197

				279.14		2.459197

				279.16		2.459197

				279.18		2.459197

				279.21		2.459197

				279.23		2.459197

				279.25		2.454797

				279.27		2.454797

				279.29		2.454797

				279.31		2.454797

				279.33		2.454797

				279.35		2.454797

				279.37		2.454797

				279.39		2.454797

				279.41		2.454797

				279.44		2.454797

				279.46		2.454797

				279.48		2.454797

				279.5		2.454797

				279.52		2.454797

				279.54		2.454797

				279.56		2.454797

				279.58		2.450398

				279.6		2.450398

				279.62		2.450398

				279.64		2.450398

				279.67		2.450398

				279.69		2.450398

				279.71		2.450398

				279.73		2.450398

				279.75		2.450398

				279.77		2.450398

				279.79		2.450398

				279.81		2.450398

				279.83		2.450398

				279.85		2.450398

				279.87		2.450398

				279.9		2.445999

				279.92		2.445999

				279.94		2.445999

				279.96		2.445999

				279.98		2.445999

				280		2.445999

				280.02		2.445999

				280.04		2.445999

				280.06		2.445999

				280.08		2.445999

				280.1		2.445999

				280.13		2.445999

				280.15		2.445999

				280.17		2.445999

				280.19		2.445999

				280.21		2.445999

				280.23		2.445999

				280.25		2.445999

				280.27		2.445999

				280.29		2.445999

				280.31		2.445999

				280.34		2.445999

				280.36		2.445999

				280.38		2.445999

				280.4		2.445999

				280.42		2.445999

				280.44		2.445999

				280.46		2.445999

				280.48		2.445999

				280.5		2.445999

				280.52		2.445999

				280.54		2.445999

				280.57		2.445999

				280.59		2.4416

				280.61		2.445999

				280.63		2.445999

				280.65		2.445999

				280.67		2.4416

				280.69		2.445999

				280.71		2.4416

				280.73		2.4416

				280.75		2.4416

				280.77		2.4416

				280.8		2.4416

				280.82		2.4416

				280.84		2.4416

				280.86		2.4416

				280.88		2.4416

				280.9		2.4416

				280.92		2.4416

				280.94		2.4416

				280.96		2.4416

				280.98		2.4416

				281		2.4416

				281.03		2.4416

				281.05		2.4416

				281.07		2.4416

				281.09		2.4416

				281.11		2.4416

				281.13		2.4416

				281.15		2.4372

				281.17		2.4372

				281.19		2.4372

				281.21		2.4372

				281.24		2.4372

				281.26		2.4372

				281.28		2.4372

				281.3		2.4372

				281.32		2.4372

				281.34		2.4372

				281.36		2.4372

				281.38		2.4372

				281.4		2.4372

				281.42		2.4372

				281.44		2.4372

				281.47		2.4372

				281.49		2.4372

				281.51		2.4372

				281.53		2.4372

				281.55		2.4372

				281.57		2.4372

				281.59		2.4372

				281.61		2.4372

				281.63		2.4372

				281.65		2.4372

				281.67		2.4372

				281.7		2.4372

				281.72		2.4372

				281.74		2.4372

				281.76		2.432801

				281.78		2.4372

				281.8		2.432801

				281.82		2.432801

				281.84		2.432801

				281.86		2.432801

				281.88		2.432801

				281.91		2.432801

				281.93		2.432801

				281.95		2.432801

				281.97		2.432801

				281.99		2.432801

				282.01		2.432801

				282.03		2.432801

				282.05		2.432801

				282.07		2.432801

				282.09		2.432801

				282.11		2.432801

				282.14		2.432801

				282.16		2.432801

				282.18		2.432801

				282.2		2.432801

				282.22		2.432801

				282.24		2.432801

				282.26		2.432801

				282.28		2.432801

				282.3		2.432801

				282.32		2.432801

				282.34		2.432801

				282.37		2.432801

				282.39		2.428402

				282.41		2.428402

				282.43		2.428402

				282.45		2.428402

				282.47		2.428402

				282.49		2.428402

				282.51		2.428402

				282.53		2.428402

				282.55		2.428402

				282.58		2.428402

				282.6		2.428402

				282.62		2.428402

				282.64		2.428402

				282.66		2.428402

				282.68		2.428402

				282.7		2.424002

				282.72		2.424002

				282.74		2.424002

				282.76		2.424002

				282.78		2.424002

				282.81		2.424002

				282.83		2.424002

				282.85		2.424002

				282.87		2.424002

				282.89		2.424002

				282.91		2.424002

				282.93		2.424002

				282.95		2.424002

				282.97		2.424002

				282.99		2.424002

				283.01		2.424002

				283.04		2.424002

				283.06		2.424002

				283.08		2.424002

				283.1		2.419603

				283.12		2.419603

				283.14		2.419603

				283.16		2.419603

				283.18		2.419603

				283.2		2.419603

				283.22		2.419603

				283.25		2.419603

				283.27		2.419603

				283.29		2.419603

				283.31		2.419603

				283.33		2.415204

				283.35		2.415204

				283.37		2.415204

				283.39		2.415204

				283.41		2.415204

				283.43		2.415204

				283.45		2.415204

				283.48		2.415204

				283.5		2.415204

				283.52		2.415204

				283.54		2.415204

				283.56		2.415204

				283.58		2.415204

				283.6		2.415204

				283.62		2.415204

				283.64		2.415204

				283.66		2.415204

				283.68		2.415204

				283.71		2.415204

				283.73		2.415204

				283.75		2.415204

				283.77		2.415204

				283.79		2.415204

				283.81		2.415204

				283.83		2.415204

				283.85		2.410805

				283.87		2.415204

				283.89		2.410805

				283.92		2.410805

				283.94		2.410805

				283.96		2.410805

				283.98		2.410805

				284		2.410805

				284.02		2.410805

				284.04		2.410805

				284.06		2.410805

				284.08		2.410805

				284.1		2.410805

				284.12		2.410805

				284.15		2.410805

				284.17		2.410805

				284.19		2.410805

				284.21		2.410805

				284.23		2.410805

				284.25		2.410805

				284.27		2.410805

				284.29		2.410805

				284.31		2.410805

				284.33		2.410805

				284.36		2.410805

				284.38		2.410805

				284.4		2.410805

				284.42		2.410805

				284.44		2.410805

				284.46		2.410805

				284.48		2.406405

				284.5		2.406405

				284.52		2.406405

				284.54		2.406405

				284.56		2.406405

				284.59		2.406405

				284.61		2.410805

				284.63		2.406405

				284.65		2.410805

				284.67		2.406405

				284.69		2.406405

				284.71		2.410805

				284.73		2.410805

				284.75		2.410805

				284.77		2.410805

				284.8		2.410805

				284.82		2.410805

				284.84		2.410805

				284.86		2.410805

				284.88		2.410805

				284.9		2.410805

				284.92		2.410805

				284.94		2.410805

				284.96		2.410805

				284.98		2.410805

				285.01		2.410805

				285.03		2.410805

				285.05		2.406405

				285.07		2.410805

				285.09		2.410805

				285.11		2.406405

				285.13		2.406405

				285.15		2.406405

				285.17		2.406405

				285.19		2.406405

				285.21		2.406405

				285.24		2.406405

				285.26		2.406405

				285.28		2.406405

				285.3		2.406405

				285.32		2.406405

				285.34		2.406405

				285.36		2.406405

				285.38		2.406405

				285.4		2.406405

				285.42		2.406405

				285.45		2.406405

				285.47		2.406405

				285.49		2.406405

				285.51		2.406405

				285.53		2.406405

				285.55		2.406405

				285.57		2.406405

				285.59		2.406405

				285.61		2.406405

				285.63		2.406405

				285.65		2.406405

				285.68		2.406405

				285.7		2.406405

				285.72		2.406405

				285.74		2.406405

				285.76		2.406405

				285.78		2.406405

				285.8		2.406405

				285.82		2.406405

				285.84		2.406405

				285.86		2.406405

				285.89		2.406405

				285.91		2.406405

				285.93		2.406405

				285.95		2.406405

				285.97		2.406405

				285.99		2.406405

				286.01		2.406405

				286.03		2.406405

				286.05		2.406405

				286.07		2.406405

				286.1		2.406405

				286.12		2.406405

				286.14		2.406405

				286.16		2.406405

				286.18		2.406405

				286.2		2.406405

				286.22		2.406405

				286.24		2.406405

				286.26		2.406405

				286.28		2.406405

				286.3		2.406405

				286.33		2.406405

				286.35		2.406405

				286.37		2.406405

				286.39		2.406405

				286.41		2.406405

				286.43		2.406405

				286.45		2.406405

				286.47		2.406405

				286.49		2.406405

				286.51		2.406405

				286.54		2.406405

				286.56		2.406405

				286.58		2.406405

				286.6		2.406405

				286.62		2.406405

				286.64		2.402006

				286.66		2.402006

				286.68		2.402006

				286.7		2.402006

				286.72		2.402006

				286.75		2.402006

				286.77		2.402006

				286.79		2.402006

				286.81		2.402006

				286.83		2.402006

				286.85		2.402006

				286.87		2.402006

				286.89		2.402006

				286.91		2.402006

				286.93		2.402006

				286.96		2.402006

				286.98		2.402006

				287		2.402006

				287.02		2.402006

				287.04		2.402006

				287.06		2.402006

				287.08		2.402006

				287.1		2.402006

				287.12		2.402006

				287.14		2.402006

				287.17		2.402006

				287.19		2.402006

				287.21		2.402006

				287.23		2.402006

				287.25		2.402006

				287.27		2.402006

				287.29		2.402006

				287.31		2.402006

				287.33		2.402006

				287.35		2.402006

				287.38		2.402006

				287.4		2.402006

				287.42		2.402006

				287.44		2.402006

				287.46		2.402006

				287.48		2.402006

				287.5		2.402006

				287.52		2.402006

				287.54		2.402006

				287.56		2.402006

				287.59		2.402006

				287.61		2.402006

				287.63		2.402006

				287.65		2.402006

				287.67		2.402006

				287.69		2.397607

				287.71		2.402006

				287.73		2.397607

				287.75		2.397607

				287.77		2.397607

				287.79		2.397607

				287.82		2.397607

				287.84		2.397607

				287.86		2.397607

				287.88		2.397607

				287.9		2.397607

				287.92		2.397607

				287.94		2.397607

				287.96		2.397607

				287.98		2.397607

				288		2.397607

				288.03		2.397607

				288.05		2.397607

				288.07		2.397607

				288.09		2.397607

				288.11		2.397607

				288.13		2.397607

				288.15		2.397607

				288.17		2.397607

				288.19		2.397607

				288.21		2.397607

				288.24		2.397607

				288.26		2.393208

				288.28		2.397607

				288.3		2.397607

				288.32		2.393208

				288.34		2.397607

				288.36		2.393208

				288.38		2.393208

				288.4		2.393208

				288.42		2.397607

				288.45		2.397607

				288.47		2.393208

				288.49		2.393208

				288.51		2.393208

				288.53		2.393208

				288.55		2.393208

				288.57		2.393208

				288.59		2.393208

				288.61		2.393208

				288.63		2.393208

				288.65		2.393208

				288.68		2.393208

				288.7		2.393208

				288.72		2.393208

				288.74		2.393208

				288.76		2.393208

				288.78		2.393208

				288.8		2.393208

				288.82		2.393208

				288.84		2.393208

				288.86		2.393208

				288.89		2.393208

				288.91		2.393208

				288.93		2.393208

				288.95		2.393208

				288.97		2.393208

				288.99		2.393208

				289.01		2.393208

				289.03		2.393208

				289.05		2.393208

				289.07		2.393208

				289.1		2.393208

				289.12		2.393208

				289.14		2.393208

				289.16		2.393208

				289.18		2.393208

				289.2		2.393208

				289.22		2.393208

				289.24		2.393208

				289.26		2.393208

				289.28		2.393208

				289.31		2.393208

				289.33		2.393208

				289.35		2.393208

				289.37		2.393208

				289.39		2.393208

				289.41		2.393208

				289.43		2.393208

				289.45		2.393208

				289.47		2.393208

				289.49		2.393208

				289.52		2.393208

				289.54		2.393208

				289.56		2.393208

				289.58		2.393208

				289.6		2.393208

				289.62		2.393208

				289.64		2.393208

				289.66		2.393208

				289.68		2.393208

				289.7		2.393208

				289.73		2.393208

				289.75		2.393208

				289.77		2.393208

				289.79		2.393208

				289.81		2.393208

				289.83		2.393208

				289.85		2.393208

				289.87		2.393208

				289.89		2.393208

				289.91		2.393208

				289.94		2.393208

				289.96		2.393208

				289.98		2.393208

				290		2.393208

				290.02		2.393208

				290.04		2.393208

				290.06		2.393208

				290.08		2.393208

				290.1		2.393208

				290.12		2.393208

				290.15		2.393208

				290.17		2.393208

				290.19		2.393208

				290.21		2.393208

				290.23		2.393208

				290.25		2.393208

				290.27		2.393208

				290.29		2.393208

				290.31		2.393208

				290.33		2.393208

				290.36		2.393208

				290.38		2.393208

				290.4		2.393208

				290.42		2.393208

				290.44		2.393208

				290.46		2.393208

				290.48		2.393208

				290.5		2.393208

				290.52		2.393208

				290.54		2.393208

				290.57		2.393208

				290.59		2.393208

				290.61		2.393208

				290.63		2.393208

				290.65		2.393208

				290.67		2.393208

				290.69		2.393208

				290.71		2.393208

				290.73		2.393208

				290.75		2.397607

				290.78		2.393208

				290.8		2.397607

				290.82		2.397607

				290.84		2.397607

				290.86		2.397607

				290.88		2.397607

				290.9		2.397607

				290.92		2.397607

				290.94		2.397607

				290.96		2.397607

				290.99		2.397607

				291.01		2.397607

				291.03		2.397607

				291.05		2.397607

				291.07		2.397607

				291.09		2.397607

				291.11		2.397607

				291.13		2.397607

				291.15		2.397607

				291.17		2.397607

				291.2		2.397607

				291.22		2.397607

				291.24		2.397607

				291.26		2.397607

				291.28		2.397607

				291.3		2.397607

				291.32		2.397607

				291.34		2.397607

				291.36		2.397607

				291.39		2.397607

				291.41		2.397607

				291.43		2.397607

				291.45		2.397607

				291.47		2.397607

				291.49		2.397607

				291.51		2.397607

				291.53		2.397607

				291.55		2.397607

				291.57		2.397607

				291.6		2.397607

				291.62		2.397607

				291.64		2.397607

				291.66		2.397607

				291.68		2.393208

				291.7		2.393208

				291.72		2.393208

				291.74		2.397607

				291.76		2.397607

				291.78		2.397607

				291.81		2.397607

				291.83		2.397607

				291.85		2.397607

				291.87		2.393208

				291.89		2.393208

				291.91		2.397607

				291.93		2.397607

				291.95		2.393208

				291.97		2.393208

				291.99		2.393208

				292.02		2.393208

				292.04		2.393208

				292.06		2.393208

				292.08		2.393208

				292.1		2.393208

				292.12		2.393208

				292.14		2.393208

				292.16		2.393208

				292.18		2.393208

				292.2		2.393208

				292.23		2.393208

				292.25		2.393208

				292.27		2.393208

				292.29		2.393208

				292.31		2.393208

				292.33		2.393208

				292.35		2.393208

				292.37		2.393208

				292.39		2.393208

				292.42		2.393208

				292.44		2.393208

				292.46		2.393208

				292.48		2.393208

				292.5		2.393208

				292.52		2.393208

				292.54		2.393208

				292.56		2.393208

				292.58		2.388808

				292.6		2.393208

				292.63		2.393208

				292.65		2.393208

				292.67		2.388808

				292.69		2.388808

				292.71		2.388808

				292.73		2.388808

				292.75		2.388808

				292.77		2.388808

				292.79		2.388808

				292.81		2.388808

				292.84		2.388808

				292.86		2.388808

				292.88		2.388808

				292.9		2.388808

				292.92		2.388808

				292.94		2.388808

				292.96		2.388808

				292.98		2.388808

				293		2.388808

				293.02		2.388808

				293.05		2.388808

				293.07		2.388808

				293.09		2.388808

				293.11		2.388808

				293.13		2.388808

				293.15		2.388808

				293.17		2.388808

				293.19		2.388808

				293.21		2.388808

				293.24		2.388808

				293.26		2.388808

				293.28		2.388808

				293.3		2.388808

				293.32		2.388808

				293.34		2.388808

				293.36		2.388808

				293.38		2.388808

				293.4		2.388808

				293.42		2.388808

				293.45		2.388808

				293.47		2.388808

				293.49		2.388808

				293.51		2.388808

				293.53		2.388808

				293.55		2.388808

				293.57		2.388808

				293.59		2.388808

				293.61		2.388808

				293.63		2.388808

				293.66		2.388808

				293.68		2.388808

				293.7		2.388808

				293.72		2.388808

				293.74		2.393208

				293.76		2.393208

				293.78		2.393208

				293.8		2.393208

				293.82		2.393208

				293.85		2.393208

				293.87		2.393208

				293.89		2.393208

				293.91		2.393208

				293.93		2.393208

				293.95		2.393208

				293.97		2.393208

				293.99		2.393208

				294.01		2.393208

				294.03		2.393208

				294.06		2.393208

				294.08		2.393208

				294.1		2.393208

				294.12		2.393208

				294.14		2.393208

				294.16		2.393208

				294.18		2.393208

				294.2		2.393208

				294.22		2.393208

				294.25		2.393208

				294.27		2.393208

				294.29		2.393208

				294.31		2.393208

				294.33		2.393208

				294.35		2.393208

				294.37		2.393208

				294.39		2.393208

				294.41		2.393208

				294.43		2.393208

				294.46		2.393208

				294.48		2.393208

				294.5		2.393208

				294.52		2.393208

				294.54		2.393208

				294.56		2.393208

				294.58		2.393208

				294.6		2.393208

				294.62		2.393208

				294.65		2.393208

				294.67		2.393208

				294.69		2.393208

				294.71		2.393208

				294.73		2.393208

				294.75		2.393208

				294.77		2.393208

				294.79		2.393208

				294.81		2.397607

				294.83		2.397607

				294.86		2.397607

				294.88		2.397607

				294.9		2.397607

				294.92		2.397607

				294.94		2.397607

				294.96		2.397607

				294.98		2.397607

				295		2.397607

				295.02		2.393208

				295.05		2.393208

				295.07		2.393208

				295.09		2.393208

				295.11		2.393208

				295.13		2.393208

				295.15		2.393208

				295.17		2.393208

				295.19		2.393208

				295.21		2.393208

				295.23		2.393208

				295.26		2.393208

				295.28		2.393208

				295.3		2.393208

				295.32		2.393208

				295.34		2.393208

				295.36		2.393208

				295.38		2.393208

				295.4		2.393208

				295.42		2.393208

				295.45		2.393208

				295.47		2.393208

				295.49		2.397607

				295.51		2.393208

				295.53		2.393208

				295.55		2.393208

				295.57		2.393208

				295.59		2.393208

				295.61		2.393208

				295.63		2.393208

				295.66		2.393208

				295.68		2.393208

				295.7		2.393208

				295.72		2.393208

				295.74		2.393208

				295.76		2.393208

				295.78		2.393208

				295.8		2.393208

				295.82		2.393208

				295.85		2.393208

				295.87		2.393208

				295.89		2.393208

				295.91		2.393208

				295.93		2.393208

				295.95		2.393208

				295.97		2.393208

				295.99		2.393208

				296.01		2.393208

				296.03		2.393208

				296.06		2.393208

				296.08		2.388808

				296.1		2.388808

				296.12		2.388808

				296.14		2.388808

				296.16		2.388808

				296.18		2.388808

				296.2		2.388808

				296.22		2.388808

				296.24		2.388808

				296.27		2.388808

				296.29		2.388808

				296.31		2.388808

				296.33		2.388808

				296.35		2.388808

				296.37		2.388808

				296.39		2.388808

				296.41		2.388808

				296.43		2.388808

				296.46		2.388808

				296.48		2.388808

				296.5		2.388808

				296.52		2.388808

				296.54		2.388808

				296.56		2.388808

				296.58		2.388808

				296.6		2.388808

				296.62		2.388808

				296.64		2.388808

				296.67		2.384409

				296.69		2.384409

				296.71		2.388808

				296.73		2.384409

				296.75		2.384409

				296.77		2.384409

				296.79		2.384409

				296.81		2.384409

				296.83		2.384409

				296.85		2.384409

				296.88		2.384409

				296.9		2.384409

				296.92		2.384409

				296.94		2.384409

				296.96		2.384409

				296.98		2.384409

				297		2.384409

				297.02		2.38001

				297.04		2.38001

				297.07		2.38001

				297.09		2.38001

				297.11		2.38001

				297.13		2.38001

				297.15		2.38001

				297.17		2.38001

				297.19		2.38001

				297.21		2.38001

				297.23		2.38001

				297.26		2.38001

				297.28		2.38001

				297.3		2.38001

				297.32		2.38001

				297.34		2.38001

				297.36		2.38001

				297.38		2.38001

				297.4		2.38001

				297.42		2.38001

				297.44		2.38001

				297.47		2.38001

				297.49		2.38001

				297.51		2.38001

				297.53		2.38001

				297.55		2.38001

				297.57		2.37561

				297.59		2.38001

				297.61		2.37561

				297.63		2.37561

				297.66		2.37561

				297.68		2.37561

				297.7		2.37561

				297.72		2.37561

				297.74		2.37561

				297.76		2.37561

				297.78		2.37561

				297.8		2.37561

				297.82		2.37561

				297.85		2.37561

				297.87		2.37561

				297.89		2.37561

				297.91		2.37561

				297.93		2.37561

				297.95		2.37561

				297.97		2.37561

				297.99		2.37561

				298.01		2.37561

				298.04		2.37561

				298.06		2.37561

				298.08		2.37561

				298.1		2.37561

				298.12		2.37561

				298.14		2.37561

				298.16		2.37561

				298.18		2.37561

				298.2		2.37561

				298.22		2.37561

				298.25		2.37561

				298.27		2.37561

				298.29		2.37561

				298.31		2.37561

				298.33		2.371211

				298.35		2.37561

				298.37		2.37561

				298.39		2.37561

				298.41		2.37561

				298.44		2.37561

				298.46		2.37561

				298.48		2.37561

				298.5		2.37561

				298.52		2.37561

				298.54		2.37561

				298.56		2.37561

				298.58		2.37561

				298.6		2.37561

				298.62		2.37561

				298.65		2.37561

				298.67		2.37561

				298.69		2.37561

				298.71		2.37561

				298.73		2.37561

				298.75		2.37561

				298.77		2.37561

				298.79		2.37561

				298.81		2.37561

				298.84		2.37561

				298.86		2.37561

				298.88		2.37561

				298.9		2.37561

				298.92		2.37561

				298.94		2.37561

				298.96		2.37561

				298.98		2.37561

				299		2.37561

				299.02		2.37561

				299.05		2.37561

				299.07		2.37561

				299.09		2.37561

				299.11		2.38001

				299.13		2.38001

				299.15		2.38001

				299.17		2.38001

				299.19		2.38001

				299.21		2.38001

				299.24		2.38001

				299.26		2.38001

				299.28		2.38001

				299.3		2.38001

				299.32		2.38001

				299.34		2.38001

				299.36		2.38001

				299.38		2.38001

				299.4		2.38001

				299.42		2.38001

				299.45		2.38001

				299.47		2.38001

				299.49		2.38001

				299.51		2.38001

				299.53		2.38001

				299.55		2.38001

				299.57		2.38001

				299.59		2.38001

				299.61		2.38001

				299.64		2.38001

				299.66		2.38001

				299.68		2.38001

				299.7		2.38001

				299.72		2.38001

				299.74		2.38001

				299.76		2.38001

				299.78		2.38001

				299.8		2.38001

				299.83		2.38001

				299.85		2.38001

				299.87		2.38001

				299.89		2.38001

				299.91		2.38001

				299.93		2.38001

				299.95		2.38001

				299.97		2.38001

				299.99		2.38001

				300.01		2.38001

				300.04		2.38001

				300.06		2.38001

				300.08		2.38001

				300.1		2.38001

				300.12		2.38001

				300.14		2.38001

				300.16		2.38001

				300.18		2.38001

				300.2		2.38001

				300.23		2.38001

				300.25		2.384409

				300.27		2.38001

				300.29		2.38001

				300.31		2.38001

				300.33		2.38001

				300.35		2.384409

				300.37		2.384409

				300.39		2.384409

				300.41		2.384409

				300.44		2.384409

				300.46		2.384409

				300.48		2.38001

				300.5		2.384409

				300.52		2.384409

				300.54		2.384409

				300.56		2.384409

				300.58		2.384409

				300.6		2.384409

				300.63		2.384409

				300.65		2.384409

				300.67		2.384409

				300.69		2.384409

				300.71		2.384409

				300.73		2.384409

				300.75		2.384409

				300.77		2.384409

				300.79		2.384409

				300.81		2.384409

				300.84		2.384409

				300.86		2.38001

				300.88		2.384409

				300.9		2.384409

				300.92		2.384409

				300.94		2.38001

				300.96		2.384409

				300.98		2.384409

				301		2.38001

				301.03		2.38001

				301.05		2.38001

				301.07		2.38001

				301.09		2.38001

				301.11		2.38001

				301.13		2.38001

				301.15		2.38001

				301.17		2.38001

				301.19		2.38001

				301.22		2.38001

				301.24		2.38001

				301.26		2.38001

				301.28		2.38001

				301.3		2.38001

				301.32		2.38001

				301.34		2.38001

				301.36		2.38001

				301.38		2.37561

				301.41		2.37561

				301.43		2.37561

				301.45		2.37561

				301.47		2.37561

				301.49		2.37561

				301.51		2.37561

				301.53		2.37561

				301.55		2.37561

				301.57		2.37561

				301.6		2.37561

				301.62		2.37561

				301.64		2.37561

				301.66		2.37561

				301.68		2.37561

				301.7		2.37561

				301.72		2.37561

				301.74		2.37561

				301.76		2.37561

				301.79		2.37561

				301.81		2.37561

				301.83		2.37561

				301.85		2.37561

				301.87		2.37561

				301.89		2.37561

				301.91		2.37561

				301.93		2.37561

				301.95		2.37561

				301.97		2.37561

				302		2.37561

				302.02		2.37561

				302.04		2.37561

				302.06		2.37561

				302.08		2.37561

				302.1		2.37561

				302.12		2.37561

				302.14		2.37561

				302.16		2.37561

				302.19		2.37561

				302.21		2.37561

				302.23		2.37561

				302.25		2.37561

				302.27		2.37561

				302.29		2.37561

				302.31		2.37561

				302.33		2.37561

				302.35		2.37561

				302.38		2.37561

				302.4		2.371211

				302.42		2.371211

				302.44		2.371211

				302.46		2.371211

				302.48		2.371211

				302.5		2.371211

				302.52		2.371211

				302.54		2.371211

				302.57		2.371211

				302.59		2.371211

				302.61		2.371211

				302.63		2.371211

				302.65		2.371211

				302.67		2.371211

				302.69		2.371211

				302.71		2.371211

				302.73		2.371211

				302.76		2.371211

				302.78		2.371211

				302.8		2.371211

				302.82		2.371211

				302.84		2.371211

				302.86		2.371211

				302.88		2.371211

				302.9		2.371211

				302.92		2.371211

				302.95		2.371211

				302.97		2.371211

				302.99		2.371211

				303.01		2.371211

				303.03		2.371211

				303.05		2.371211

				303.07		2.371211

				303.09		2.371211

				303.11		2.371211

				303.14		2.371211

				303.16		2.371211

				303.18		2.371211

				303.2		2.371211

				303.22		2.371211

				303.24		2.371211

				303.26		2.371211

				303.28		2.371211

				303.3		2.371211

				303.33		2.371211

				303.35		2.371211

				303.37		2.371211

				303.39		2.371211

				303.41		2.371211

				303.43		2.371211

				303.45		2.371211

				303.47		2.371211

				303.49		2.371211

				303.52		2.371211

				303.54		2.371211

				303.56		2.371211

				303.58		2.371211

				303.6		2.371211

				303.62		2.371211

				303.64		2.371211

				303.66		2.371211

				303.68		2.371211

				303.7		2.371211

				303.73		2.371211

				303.75		2.371211

				303.77		2.371211

				303.79		2.371211

				303.81		2.371211

				303.83		2.371211

				303.85		2.371211

				303.87		2.371211

				303.89		2.371211

				303.92		2.371211

				303.94		2.371211

				303.96		2.371211

				303.98		2.371211

				304		2.371211

				304.02		2.371211

				304.04		2.371211

				304.06		2.371211

				304.08		2.371211

				304.11		2.371211

				304.13		2.371211

				304.15		2.371211

				304.17		2.371211

				304.19		2.371211

				304.21		2.371211

				304.23		2.371211

				304.25		2.371211

				304.27		2.371211

				304.29		2.371211

				304.32		2.371211

				304.34		2.371211

				304.36		2.371211

				304.38		2.371211

				304.4		2.371211

				304.42		2.371211

				304.44		2.371211

				304.46		2.371211

				304.48		2.371211

				304.51		2.371211

				304.53		2.371211

				304.55		2.371211

				304.57		2.371211

				304.59		2.371211

				304.61		2.371211

				304.63		2.371211

				304.65		2.371211

				304.67		2.371211

				304.7		2.371211

				304.72		2.371211

				304.74		2.371211

				304.76		2.371211

				304.78		2.371211

				304.8		2.371211

				304.82		2.371211

				304.84		2.371211

				304.86		2.371211

				304.89		2.371211

				304.91		2.371211

				304.93		2.371211

				304.95		2.371211

				304.97		2.371211

				304.99		2.371211

				305.01		2.366812

				305.03		2.366812

				305.05		2.366812

				305.08		2.371211

				305.1		2.371211

				305.12		2.371211

				305.14		2.366812

				305.16		2.371211

				305.18		2.366812

				305.2		2.366812

				305.22		2.366812

				305.24		2.366812

				305.26		2.366812

				305.29		2.366812

				305.31		2.366812

				305.33		2.366812

				305.35		2.366812

				305.37		2.366812

				305.39		2.366812

				305.41		2.366812

				305.43		2.366812

				305.45		2.366812

				305.48		2.366812

				305.5		2.366812

				305.52		2.366812

				305.54		2.366812

				305.56		2.366812

				305.58		2.366812

				305.6		2.366812

				305.62		2.366812

				305.64		2.366812

				305.66		2.366812

				305.69		2.366812

				305.71		2.366812

				305.73		2.366812

				305.75		2.366812

				305.77		2.366812

				305.79		2.366812

				305.81		2.366812

				305.83		2.366812

				305.85		2.366812

				305.88		2.366812

				305.9		2.366812

				305.92		2.366812

				305.94		2.366812

				305.96		2.366812

				305.98		2.366812

				306		2.366812

				306.02		2.366812

				306.04		2.366812

				306.07		2.362413

				306.09		2.366812

				306.11		2.362413

				306.13		2.362413

				306.15		2.362413

				306.17		2.366812

				306.19		2.362413

				306.21		2.366812

				306.23		2.362413

				306.25		2.362413

				306.28		2.362413

				306.3		2.362413

				306.32		2.362413

				306.34		2.362413

				306.36		2.362413

				306.38		2.362413

				306.4		2.362413

				306.42		2.362413

				306.44		2.362413

				306.47		2.362413

				306.49		2.362413

				306.51		2.362413

				306.53		2.362413

				306.55		2.362413

				306.57		2.362413

				306.59		2.362413

				306.61		2.362413

				306.63		2.362413

				306.66		2.362413

				306.68		2.362413

				306.7		2.362413

				306.72		2.362413

				306.74		2.362413

				306.76		2.362413

				306.78		2.362413

				306.8		2.362413

				306.82		2.362413

				306.85		2.362413

				306.87		2.362413

				306.89		2.362413

				306.91		2.362413

				306.93		2.362413

				306.95		2.362413

				306.97		2.362413

				306.99		2.362413

				307.01		2.362413

				307.04		2.362413

				307.06		2.362413

				307.08		2.362413

				307.1		2.362413

				307.12		2.362413

				307.14		2.362413

				307.16		2.362413

				307.18		2.358013

				307.2		2.362413

				307.23		2.362413

				307.25		2.358013

				307.27		2.362413

				307.29		2.362413

				307.31		2.362413

				307.33		2.362413

				307.35		2.362413

				307.37		2.362413

				307.39		2.362413

				307.42		2.362413

				307.44		2.362413

				307.46		2.362413

				307.48		2.362413

				307.5		2.362413

				307.52		2.362413

				307.54		2.362413

				307.56		2.362413

				307.58		2.362413

				307.61		2.362413

				307.63		2.362413

				307.65		2.362413

				307.67		2.362413

				307.69		2.362413

				307.71		2.362413

				307.73		2.362413

				307.75		2.362413

				307.77		2.362413

				307.8		2.362413

				307.82		2.362413

				307.84		2.362413

				307.86		2.362413

				307.88		2.362413

				307.9		2.362413

				307.92		2.362413

				307.94		2.362413

				307.96		2.362413

				307.99		2.362413

				308.01		2.362413

				308.03		2.362413

				308.05		2.366812

				308.07		2.366812

				308.09		2.366812

				308.11		2.366812

				308.13		2.366812

				308.15		2.362413

				308.18		2.362413

				308.2		2.362413

				308.22		2.362413

				308.24		2.362413

				308.26		2.362413

				308.28		2.366812

				308.3		2.366812

				308.32		2.366812

				308.34		2.366812

				308.37		2.366812

				308.39		2.366812

				308.41		2.366812

				308.43		2.366812

				308.45		2.366812

				308.47		2.366812

				308.49		2.366812

				308.51		2.366812

				308.53		2.366812

				308.56		2.366812

				308.58		2.366812

				308.6		2.366812

				308.62		2.366812

				308.64		2.366812

				308.66		2.366812

				308.68		2.366812

				308.7		2.366812

				308.72		2.366812

				308.74		2.366812

				308.77		2.366812

				308.79		2.366812

				308.81		2.366812

				308.83		2.366812

				308.85		2.366812

				308.87		2.366812

				308.89		2.366812

				308.91		2.366812

				308.93		2.366812

				308.96		2.366812

				308.98		2.366812

				309		2.366812

				309.02		2.366812

				309.04		2.366812

				309.06		2.366812

				309.08		2.366812

				309.1		2.366812

				309.12		2.366812

				309.15		2.366812

				309.17		2.366812

				309.19		2.366812

				309.21		2.366812

				309.23		2.366812

				309.25		2.366812

				309.27		2.366812

				309.29		2.366812

				309.31		2.366812

				309.34		2.366812

				309.36		2.366812

				309.38		2.366812

				309.4		2.366812

				309.42		2.366812

				309.44		2.366812

				309.46		2.366812

				309.48		2.366812

				309.5		2.366812

				309.52		2.366812

				309.55		2.366812

				309.57		2.366812

				309.59		2.366812

				309.61		2.366812

				309.63		2.366812

				309.65		2.366812

				309.67		2.366812

				309.69		2.366812

				309.71		2.362413

				309.74		2.362413

				309.76		2.362413

				309.78		2.362413

				309.8		2.362413

				309.82		2.362413

				309.84		2.362413

				309.86		2.362413

				309.88		2.362413

				309.9		2.362413

				309.93		2.362413

				309.95		2.362413

				309.97		2.362413

				309.99		2.362413

				310.01		2.362413

				310.03		2.362413

				310.05		2.362413

				310.07		2.362413

				310.09		2.362413

				310.12		2.362413

				310.14		2.362413

				310.16		2.362413

				310.18		2.362413

				310.2		2.362413

				310.22		2.362413

				310.24		2.362413

				310.26		2.362413

				310.28		2.362413

				310.31		2.362413

				310.33		2.362413

				310.35		2.362413

				310.37		2.362413

				310.39		2.362413

				310.41		2.362413

				310.43		2.362413

				310.45		2.362413

				310.47		2.358013

				310.49		2.362413

				310.52		2.358013

				310.54		2.358013

				310.56		2.358013

				310.58		2.358013

				310.6		2.358013

				310.62		2.358013

				310.64		2.358013

				310.66		2.358013

				310.68		2.358013

				310.71		2.358013

				310.73		2.358013

				310.75		2.358013

				310.77		2.358013

				310.79		2.358013

				310.81		2.358013

				310.83		2.358013

				310.85		2.358013

				310.87		2.358013

				310.9		2.358013

				310.92		2.358013

				310.94		2.358013

				310.96		2.358013

				310.98		2.358013

				311		2.358013

				311.02		2.358013

				311.04		2.358013

				311.06		2.358013

				311.09		2.358013

				311.11		2.358013

				311.13		2.358013

				311.15		2.358013

				311.17		2.358013

				311.19		2.358013

				311.21		2.358013

				311.23		2.358013

				311.25		2.358013

				311.27		2.358013

				311.3		2.358013

				311.32		2.358013

				311.34		2.358013

				311.36		2.353614

				311.38		2.353614

				311.4		2.353614

				311.42		2.353614

				311.44		2.353614

				311.46		2.353614

				311.49		2.353614

				311.51		2.353614

				311.53		2.353614

				311.55		2.353614

				311.57		2.353614

				311.59		2.353614

				311.61		2.353614

				311.63		2.353614

				311.65		2.353614

				311.68		2.353614

				311.7		2.353614

				311.72		2.353614

				311.74		2.353614

				311.76		2.353614

				311.78		2.353614

				311.8		2.358013

				311.82		2.358013

				311.84		2.358013

				311.86		2.358013

				311.89		2.358013

				311.91		2.358013

				311.93		2.358013

				311.95		2.358013

				311.97		2.358013

				311.99		2.358013

				312.01		2.358013

				312.03		2.358013

				312.05		2.358013

				312.08		2.358013

				312.1		2.358013

				312.12		2.358013

				312.14		2.358013

				312.16		2.358013

				312.18		2.358013

				312.2		2.358013

				312.22		2.358013

				312.24		2.358013

				312.27		2.358013

				312.29		2.358013

				312.31		2.358013

				312.33		2.358013

				312.35		2.358013

				312.37		2.358013

				312.39		2.358013

				312.41		2.358013

				312.43		2.358013

				312.46		2.358013

				312.48		2.358013

				312.5		2.358013

				312.52		2.358013

				312.54		2.358013

				312.56		2.358013

				312.58		2.358013

				312.6		2.358013

				312.62		2.358013

				312.65		2.358013

				312.67		2.358013

				312.69		2.358013

				312.71		2.358013

				312.73		2.358013

				312.75		2.358013

				312.77		2.358013

				312.79		2.358013

				312.81		2.358013

				312.84		2.358013

				312.86		2.358013

				312.88		2.358013

				312.9		2.358013

				312.92		2.358013

				312.94		2.358013

				312.96		2.358013

				312.98		2.358013

				313		2.358013

				313.03		2.358013

				313.05		2.358013

				313.07		2.358013

				313.09		2.358013

				313.11		2.358013

				313.13		2.358013

				313.15		2.358013

				313.17		2.358013

				313.19		2.358013

				313.22		2.358013

				313.24		2.358013

				313.26		2.358013

				313.28		2.362413

				313.3		2.362413

				313.32		2.362413

				313.34		2.362413

				313.36		2.362413

				313.39		2.362413

				313.41		2.362413

				313.43		2.362413

				313.45		2.362413

				313.47		2.362413

				313.49		2.362413

				313.51		2.362413

				313.53		2.362413

				313.55		2.362413

				313.58		2.362413

				313.6		2.362413

				313.62		2.362413

				313.64		2.362413

				313.66		2.362413

				313.68		2.362413

				313.7		2.362413

				313.72		2.362413

				313.74		2.362413

				313.77		2.362413

				313.79		2.362413

				313.81		2.362413

				313.83		2.366812

				313.85		2.366812

				313.87		2.366812

				313.89		2.366812

				313.91		2.366812

				313.93		2.366812

				313.96		2.366812

				313.98		2.366812

				314		2.366812

				314.02		2.366812

				314.04		2.366812

				314.06		2.366812

				314.08		2.366812

				314.1		2.366812

				314.12		2.366812

				314.15		2.366812

				314.17		2.366812

				314.19		2.366812

				314.21		2.366812

				314.23		2.366812

				314.25		2.366812

				314.27		2.366812

				314.29		2.366812

				314.31		2.366812

				314.34		2.366812

				314.36		2.366812

				314.38		2.366812

				314.4		2.366812

				314.42		2.366812

				314.44		2.366812

				314.46		2.366812

				314.48		2.366812

				314.5		2.366812

				314.53		2.366812

				314.55		2.366812

				314.57		2.366812

				314.59		2.366812

				314.61		2.366812

				314.63		2.366812

				314.65		2.366812

				314.67		2.366812

				314.69		2.366812

				314.72		2.366812

				314.74		2.366812

				314.76		2.366812

				314.78		2.366812

				314.8		2.366812

				314.82		2.366812

				314.84		2.366812

				314.86		2.366812

				314.88		2.366812

				314.91		2.366812

				314.93		2.366812

				314.95		2.366812

				314.97		2.366812

				314.99		2.366812

				315.01		2.366812

				315.03		2.366812

				315.05		2.366812

				315.08		2.366812

				315.1		2.366812

				315.12		2.366812

				315.14		2.366812

				315.16		2.366812

				315.18		2.366812

				315.2		2.366812

				315.22		2.366812

				315.24		2.366812

				315.27		2.371211

				315.29		2.371211

				315.31		2.371211

				315.33		2.371211

				315.35		2.371211

				315.37		2.371211

				315.39		2.371211

				315.41		2.371211

				315.43		2.371211

				315.46		2.371211

				315.48		2.371211

				315.5		2.371211

				315.52		2.371211

				315.54		2.371211

				315.56		2.371211

				315.58		2.371211

				315.6		2.371211

				315.62		2.371211

				315.65		2.371211

				315.67		2.371211

				315.69		2.371211

				315.71		2.371211

				315.73		2.371211

				315.75		2.371211

				315.77		2.371211

				315.79		2.371211

				315.81		2.371211

				315.84		2.371211

				315.86		2.371211

				315.88		2.371211

				315.9		2.371211

				315.92		2.371211

				315.94		2.371211

				315.96		2.371211

				315.98		2.366812

				316.01		2.366812

				316.03		2.366812

				316.05		2.366812

				316.07		2.366812

				316.09		2.366812

				316.11		2.366812

				316.13		2.366812

				316.15		2.366812

				316.17		2.366812

				316.2		2.366812

				316.22		2.366812

				316.24		2.366812

				316.26		2.366812

				316.28		2.366812

				316.3		2.366812

				316.32		2.366812

				316.34		2.366812

				316.37		2.366812

				316.39		2.366812

				316.41		2.366812

				316.43		2.366812

				316.45		2.366812

				316.47		2.366812

				316.49		2.366812

				316.51		2.366812

				316.53		2.366812

				316.56		2.366812

				316.58		2.366812

				316.6		2.366812

				316.62		2.366812

				316.64		2.366812

				316.66		2.366812

				316.68		2.366812

				316.7		2.366812

				316.72		2.366812

				316.75		2.366812

				316.77		2.366812

				316.79		2.366812

				316.81		2.366812

				316.83		2.366812

				316.85		2.366812

				316.87		2.366812

				316.89		2.366812

				316.92		2.366812

				316.94		2.366812

				316.96		2.366812

				316.98		2.366812

				317		2.366812

				317.02		2.366812

				317.04		2.366812

				317.06		2.366812

				317.08		2.366812

				317.11		2.366812

				317.13		2.366812

				317.15		2.366812

				317.17		2.366812

				317.19		2.366812

				317.21		2.366812

				317.23		2.366812

				317.25		2.366812

				317.27		2.366812

				317.3		2.366812

				317.32		2.366812

				317.34		2.366812

				317.36		2.366812

				317.38		2.366812

				317.4		2.366812

				317.42		2.366812

				317.44		2.366812

				317.46		2.366812

				317.49		2.366812

				317.51		2.366812

				317.53		2.366812

				317.55		2.362413

				317.57		2.362413

				317.59		2.362413

				317.61		2.362413

				317.63		2.362413

				317.66		2.362413

				317.68		2.362413

				317.7		2.362413

				317.72		2.362413

				317.74		2.362413

				317.76		2.362413

				317.78		2.362413

				317.8		2.362413

				317.82		2.362413

				317.85		2.362413

				317.87		2.362413

				317.89		2.362413

				317.91		2.362413

				317.93		2.362413

				317.95		2.362413

				317.97		2.362413

				317.99		2.362413

				318.01		2.358013

				318.04		2.358013

				318.06		2.358013

				318.08		2.358013

				318.1		2.358013

				318.12		2.358013

				318.14		2.358013

				318.16		2.358013

				318.18		2.358013

				318.21		2.358013

				318.23		2.358013

				318.25		2.358013

				318.27		2.358013

				318.29		2.358013

				318.31		2.358013

				318.33		2.358013

				318.35		2.358013

				318.37		2.358013

				318.4		2.358013

				318.42		2.358013

				318.44		2.358013

				318.46		2.358013

				318.48		2.358013

				318.5		2.358013

				318.52		2.358013

				318.54		2.358013

				318.56		2.358013

				318.59		2.358013

				318.61		2.358013

				318.63		2.358013

				318.65		2.358013

				318.67		2.358013

				318.69		2.358013

				318.71		2.358013

				318.73		2.358013

				318.75		2.358013

				318.78		2.358013

				318.8		2.358013

				318.82		2.358013

				318.84		2.358013

				318.86		2.358013

				318.88		2.358013

				318.9		2.358013

				318.92		2.358013

				318.95		2.358013

				318.97		2.358013

				318.99		2.358013

				319.01		2.358013

				319.03		2.358013

				319.05		2.358013

				319.07		2.358013

				319.09		2.358013

				319.11		2.353614

				319.14		2.353614

				319.16		2.353614

				319.18		2.353614

				319.2		2.353614

				319.22		2.353614

				319.24		2.353614

				319.26		2.353614

				319.28		2.353614

				319.3		2.353614

				319.33		2.353614

				319.35		2.353614

				319.37		2.353614

				319.39		2.353614

				319.41		2.353614

				319.43		2.353614

				319.45		2.353614

				319.47		2.353614

				319.49		2.353614

				319.52		2.353614

				319.54		2.353614

				319.56		2.353614

				319.58		2.349215

				319.6		2.349215

				319.62		2.349215

				319.64		2.349215

				319.66		2.349215

				319.69		2.349215

				319.71		2.349215

				319.73		2.349215

				319.75		2.349215

				319.77		2.349215

				319.79		2.349215

				319.81		2.349215

				319.83		2.349215

				319.85		2.349215

				319.88		2.349215

				319.9		2.349215

				319.92		2.349215

				319.94		2.349215

				319.96		2.353614

				319.98		2.353614

				320		2.353614

				320.02		2.349215

				320.04		2.349215

				320.07		2.353614

				320.09		2.353614

				320.11		2.353614

				320.13		2.353614

				320.15		2.353614

				320.17		2.353614

				320.19		2.353614

				320.21		2.353614

				320.23		2.353614

				320.26		2.353614

				320.28		2.353614

				320.3		2.353614

				320.32		2.353614

				320.34		2.353614

				320.36		2.353614

				320.38		2.353614

				320.4		2.353614

				320.42		2.353614

				320.45		2.353614

				320.47		2.353614

				320.49		2.353614

				320.51		2.353614

				320.53		2.353614

				320.55		2.353614

				320.57		2.353614

				320.59		2.353614

				320.62		2.353614

				320.64		2.353614

				320.66		2.353614

				320.68		2.353614

				320.7		2.353614

				320.72		2.353614

				320.74		2.349215

				320.76		2.353614

				320.78		2.349215

				320.81		2.349215

				320.83		2.353614

				320.85		2.349215

				320.87		2.349215

				320.89		2.349215

				320.91		2.349215

				320.93		2.353614

				320.95		2.349215

				320.97		2.349215

				321		2.349215

				321.02		2.349215

				321.04		2.349215

				321.06		2.349215

				321.08		2.353614

				321.1		2.353614

				321.12		2.349215

				321.14		2.353614

				321.16		2.349215

				321.19		2.353614

				321.21		2.353614

				321.23		2.353614

				321.25		2.353614

				321.27		2.353614

				321.29		2.353614

				321.31		2.353614

				321.33		2.353614

				321.36		2.353614

				321.38		2.353614

				321.4		2.353614

				321.42		2.353614

				321.44		2.353614

				321.46		2.353614

				321.48		2.353614

				321.5		2.353614

				321.52		2.353614

				321.55		2.353614

				321.57		2.353614

				321.59		2.353614

				321.61		2.353614

				321.63		2.353614

				321.65		2.353614

				321.67		2.353614

				321.69		2.353614

				321.71		2.353614

				321.74		2.353614

				321.76		2.353614

				321.78		2.353614

				321.8		2.353614

				321.82		2.353614

				321.84		2.353614

				321.86		2.353614

				321.88		2.353614

				321.91		2.353614

				321.93		2.353614

				321.95		2.353614

				321.97		2.353614

				321.99		2.353614

				322.01		2.353614

				322.03		2.353614

				322.05		2.353614

				322.07		2.353614

				322.1		2.353614

				322.12		2.353614

				322.14		2.353614

				322.16		2.353614

				322.18		2.353614

				322.2		2.353614

				322.22		2.353614

				322.24		2.353614

				322.27		2.353614

				322.29		2.353614

				322.31		2.353614

				322.33		2.353614

				322.35		2.353614

				322.37		2.353614

				322.39		2.353614

				322.41		2.353614

				322.43		2.353614

				322.46		2.353614

				322.48		2.353614

				322.5		2.353614

				322.52		2.353614

				322.54		2.353614

				322.56		2.353614

				322.58		2.353614

				322.6		2.353614

				322.63		2.353614

				322.65		2.353614

				322.67		2.353614

				322.69		2.353614

				322.71		2.353614

				322.73		2.353614

				322.75		2.353614

				322.77		2.353614

				322.79		2.353614

				322.82		2.353614

				322.84		2.353614

				322.86		2.353614

				322.88		2.353614

				322.9		2.353614

				322.92		2.353614

				322.94		2.353614

				322.96		2.353614

				322.99		2.353614

				323.01		2.353614

				323.03		2.353614

				323.05		2.353614

				323.07		2.353614

				323.09		2.353614

				323.11		2.353614

				323.13		2.353614

				323.15		2.353614

				323.18		2.353614

				323.2		2.353614

				323.22		2.353614

				323.24		2.353614

				323.26		2.353614

				323.28		2.353614

				323.3		2.353614

				323.32		2.349215

				323.35		2.353614

				323.37		2.353614

				323.39		2.349215

				323.41		2.353614

				323.43		2.349215

				323.45		2.349215

				323.47		2.349215

				323.49		2.349215

				323.51		2.349215

				323.54		2.349215

				323.56		2.349215

				323.58		2.349215

				323.6		2.349215

				323.62		2.349215

				323.64		2.349215

				323.66		2.349215

				323.68		2.349215

				323.71		2.349215

				323.73		2.349215

				323.75		2.349215

				323.77		2.349215

				323.79		2.349215

				323.81		2.349215

				323.83		2.349215

				323.85		2.349215

				323.87		2.349215

				323.9		2.349215

				323.92		2.349215

				323.94		2.349215

				323.96		2.349215

				323.98		2.349215

				324		2.349215

				324.02		2.349215

				324.04		2.349215

				324.07		2.349215

				324.09		2.349215

				324.11		2.349215

				324.13		2.349215

				324.15		2.349215

				324.17		2.349215

				324.19		2.349215

				324.21		2.349215

				324.24		2.349215

				324.26		2.349215

				324.28		2.349215

				324.3		2.349215

				324.32		2.349215

				324.34		2.349215

				324.36		2.349215

				324.38		2.349215

				324.4		2.349215

				324.43		2.349215

				324.45		2.349215

				324.47		2.349215

				324.49		2.349215

				324.51		2.353614

				324.53		2.353614

				324.55		2.349215

				324.57		2.353614

				324.59		2.353614

				324.62		2.353614

				324.64		2.353614

				324.66		2.353614

				324.68		2.353614

				324.7		2.353614

				324.72		2.353614

				324.74		2.353614

				324.76		2.353614

				324.79		2.353614

				324.81		2.353614

				324.83		2.353614

				324.85		2.353614

				324.87		2.353614

				324.89		2.353614

				324.91		2.353614

				324.93		2.353614

				324.95		2.353614

				324.98		2.353614

				325		2.353614

				325.02		2.353614

				325.04		2.353614

				325.06		2.353614

				325.08		2.353614

				325.1		2.353614

				325.12		2.353614

				325.15		2.353614

				325.17		2.353614

				325.19		2.353614

				325.21		2.353614

				325.23		2.353614

				325.25		2.353614

				325.27		2.353614

				325.29		2.353614

				325.32		2.353614

				325.34		2.353614

				325.36		2.353614

				325.38		2.353614

				325.4		2.353614

				325.42		2.353614

				325.44		2.353614

				325.46		2.353614

				325.48		2.353614

				325.51		2.353614

				325.53		2.353614

				325.55		2.353614

				325.57		2.353614

				325.59		2.353614

				325.61		2.353614

				325.63		2.353614

				325.65		2.353614

				325.68		2.353614

				325.7		2.353614

				325.72		2.353614

				325.74		2.353614

				325.76		2.353614

				325.78		2.353614

				325.8		2.353614

				325.82		2.353614

				325.85		2.353614

				325.87		2.353614

				325.89		2.353614

				325.91		2.353614

				325.93		2.353614

				325.95		2.353614

				325.97		2.353614

				325.99		2.353614

				326.01		2.353614

				326.04		2.353614

				326.06		2.353614

				326.08		2.349215

				326.1		2.349215

				326.12		2.349215

				326.14		2.349215

				326.16		2.349215

				326.18		2.349215

				326.21		2.349215

				326.23		2.349215

				326.25		2.349215

				326.27		2.349215

				326.29		2.349215

				326.31		2.349215

				326.33		2.349215

				326.35		2.349215

				326.37		2.349215

				326.4		2.349215

				326.42		2.349215

				326.44		2.349215

				326.46		2.349215

				326.48		2.349215

				326.5		2.349215

				326.52		2.349215

				326.54		2.349215

				326.57		2.349215

				326.59		2.349215

				326.61		2.349215

				326.63		2.349215

				326.65		2.349215

				326.67		2.349215

				326.69		2.349215

				326.71		2.349215

				326.73		2.349215

				326.76		2.349215

				326.78		2.349215

				326.8		2.349215

				326.82		2.349215

				326.84		2.349215

				326.86		2.349215

				326.88		2.349215

				326.9		2.349215

				326.93		2.349215

				326.95		2.349215

				326.97		2.349215

				326.99		2.349215

				327.01		2.349215

				327.03		2.349215

				327.05		2.349215

				327.07		2.349215

				327.09		2.349215

				327.12		2.349215

				327.14		2.349215

				327.16		2.349215

				327.18		2.349215

				327.2		2.349215

				327.22		2.349215

				327.24		2.349215

				327.26		2.349215

				327.29		2.349215

				327.31		2.349215

				327.33		2.349215

				327.35		2.349215

				327.37		2.349215

				327.39		2.349215

				327.41		2.349215

				327.43		2.349215

				327.45		2.349215

				327.48		2.349215

				327.5		2.349215

				327.52		2.349215

				327.54		2.349215

				327.56		2.349215

				327.58		2.349215

				327.6		2.349215

				327.62		2.349215

				327.65		2.349215

				327.67		2.349215

				327.69		2.344815

				327.71		2.349215

				327.73		2.349215

				327.75		2.344815

				327.77		2.349215

				327.79		2.349215

				327.81		2.349215

				327.84		2.349215

				327.86		2.349215

				327.88		2.349215

				327.9		2.349215

				327.92		2.349215

				327.94		2.349215

				327.96		2.349215

				327.98		2.349215

				328.01		2.349215

				328.03		2.349215

				328.05		2.349215

				328.07		2.349215

				328.09		2.349215

				328.11		2.349215

				328.13		2.349215

				328.15		2.349215

				328.17		2.349215

				328.2		2.349215

				328.22		2.349215

				328.24		2.349215

				328.26		2.349215

				328.28		2.349215

				328.3		2.349215

				328.32		2.349215

				328.34		2.349215

				328.36		2.349215

				328.39		2.349215

				328.41		2.349215

				328.43		2.349215

				328.45		2.349215

				328.47		2.349215

				328.49		2.349215

				328.51		2.349215

				328.53		2.349215

				328.56		2.349215

				328.58		2.349215

				328.6		2.349215

				328.62		2.349215

				328.64		2.349215

				328.66		2.349215

				328.68		2.349215

				328.7		2.349215

				328.72		2.344815

				328.75		2.349215

				328.77		2.349215

				328.79		2.349215

				328.81		2.349215

				328.83		2.349215

				328.85		2.349215

				328.87		2.349215

				328.89		2.349215

				328.91		2.349215

				328.94		2.349215

				328.96		2.349215

				328.98		2.349215

				329		2.349215

				329.02		2.349215

				329.04		2.349215

				329.06		2.349215

				329.08		2.349215

				329.11		2.344815

				329.13		2.344815

				329.15		2.344815

				329.17		2.344815

				329.19		2.344815

				329.21		2.344815

				329.23		2.344815

				329.25		2.344815

				329.27		2.344815

				329.3		2.344815

				329.32		2.344815

				329.34		2.344815

				329.36		2.344815

				329.38		2.344815

				329.4		2.344815

				329.42		2.344815

				329.44		2.344815

				329.47		2.344815

				329.49		2.344815

				329.51		2.344815

				329.53		2.344815

				329.55		2.344815

				329.57		2.344815

				329.59		2.344815

				329.61		2.344815

				329.63		2.344815

				329.66		2.344815

				329.68		2.344815

				329.7		2.344815

				329.72		2.344815

				329.74		2.344815

				329.76		2.344815

				329.78		2.344815

				329.8		2.344815

				329.82		2.344815

				329.85		2.344815

				329.87		2.344815

				329.89		2.344815

				329.91		2.344815

				329.93		2.344815

				329.95		2.344815

				329.97		2.344815

				329.99		2.344815

				330.01		2.344815

				330.04		2.344815

				330.06		2.344815

				330.08		2.344815

				330.1		2.344815

				330.12		2.344815

				330.14		2.344815

				330.16		2.344815

				330.18		2.344815

				330.2		2.344815

				330.23		2.344815

				330.25		2.344815

				330.27		2.344815

				330.29		2.344815

				330.31		2.344815

				330.33		2.344815

				330.35		2.344815

				330.37		2.344815

				330.39		2.344815

				330.42		2.344815

				330.44		2.344815

				330.46		2.344815

				330.48		2.344815

				330.5		2.344815

				330.52		2.344815

				330.54		2.344815

				330.56		2.349215

				330.59		2.344815

				330.61		2.349215

				330.63		2.349215

				330.65		2.349215

				330.67		2.349215

				330.69		2.349215

				330.71		2.344815

				330.73		2.349215

				330.75		2.344815

				330.78		2.349215

				330.8		2.344815

				330.82		2.349215

				330.84		2.344815

				330.86		2.349215

				330.88		2.349215

				330.9		2.349215

				330.92		2.349215

				330.94		2.349215

				330.97		2.349215

				330.99		2.349215

				331.01		2.344815

				331.03		2.344815

				331.05		2.349215

				331.07		2.349215

				331.09		2.349215

				331.11		2.349215

				331.13		2.349215

				331.16		2.349215

				331.18		2.349215

				331.2		2.349215

				331.22		2.349215

				331.24		2.349215

				331.26		2.349215

				331.28		2.349215

				331.3		2.349215

				331.32		2.349215

				331.35		2.349215

				331.37		2.349215

				331.39		2.349215

				331.41		2.349215

				331.43		2.349215

				331.45		2.349215

				331.47		2.349215

				331.49		2.349215

				331.51		2.349215

				331.54		2.349215

				331.56		2.349215

				331.58		2.349215

				331.6		2.349215

				331.62		2.349215

				331.64		2.349215

				331.66		2.349215

				331.68		2.349215

				331.7		2.349215

				331.73		2.349215

				331.75		2.349215

				331.77		2.349215

				331.79		2.349215

				331.81		2.353614

				331.83		2.353614

				331.85		2.353614

				331.87		2.353614

				331.89		2.353614

				331.92		2.353614

				331.94		2.353614

				331.96		2.353614

				331.98		2.353614

				332		2.353614

				332.02		2.353614

				332.04		2.353614

				332.06		2.353614

				332.08		2.353614

				332.1		2.353614

				332.13		2.353614

				332.15		2.353614

				332.17		2.353614

				332.19		2.353614

				332.21		2.353614

				332.23		2.353614

				332.25		2.353614

				332.27		2.353614

				332.29		2.353614

				332.32		2.353614

				332.34		2.353614

				332.36		2.353614

				332.38		2.353614

				332.4		2.353614

				332.42		2.353614

				332.44		2.353614

				332.46		2.353614

				332.49		2.353614

				332.51		2.353614

				332.53		2.353614

				332.55		2.353614

				332.57		2.353614

				332.59		2.353614

				332.61		2.353614

				332.63		2.353614

				332.65		2.353614

				332.68		2.353614

				332.7		2.353614

				332.72		2.353614

				332.74		2.353614

				332.76		2.353614

				332.78		2.353614

				332.8		2.353614

				332.82		2.358013

				332.84		2.358013

				332.87		2.358013

				332.89		2.358013

				332.91		2.358013

				332.93		2.358013

				332.95		2.358013

				332.97		2.358013

				332.99		2.358013

				333.01		2.358013

				333.03		2.358013

				333.06		2.358013

				333.08		2.358013

				333.1		2.358013

				333.12		2.358013

				333.14		2.358013

				333.16		2.358013

				333.18		2.358013

				333.2		2.358013

				333.22		2.358013

				333.25		2.358013

				333.27		2.358013

				333.29		2.358013

				333.31		2.358013

				333.33		2.358013

				333.35		2.358013

				333.37		2.358013

				333.39		2.358013

				333.41		2.358013

				333.44		2.358013

				333.46		2.358013

				333.48		2.358013

				333.5		2.358013

				333.52		2.358013

				333.54		2.358013

				333.56		2.358013

				333.58		2.358013

				333.6		2.358013

				333.62		2.358013

				333.65		2.358013

				333.67		2.358013

				333.69		2.358013

				333.71		2.358013

				333.73		2.358013

				333.75		2.358013

				333.77		2.358013

				333.79		2.358013

				333.81		2.358013

				333.84		2.358013

				333.86		2.358013

				333.88		2.358013

				333.9		2.358013

				333.92		2.358013

				333.94		2.358013

				333.96		2.358013

				333.98		2.358013

				334		2.358013

				334.03		2.358013

				334.05		2.358013

				334.07		2.358013

				334.09		2.358013

				334.11		2.358013

				334.13		2.358013

				334.15		2.358013

				334.17		2.358013

				334.19		2.358013

				334.22		2.358013

				334.24		2.358013

				334.26		2.358013

				334.28		2.358013

				334.3		2.358013

				334.32		2.353614

				334.34		2.353614

				334.36		2.353614

				334.38		2.353614

				334.41		2.353614

				334.43		2.353614

				334.45		2.353614

				334.47		2.353614

				334.49		2.353614

				334.51		2.353614

				334.53		2.353614

				334.55		2.353614

				334.57		2.353614

				334.6		2.353614

				334.62		2.353614

				334.64		2.353614

				334.66		2.353614

				334.68		2.353614

				334.7		2.353614

				334.72		2.349215

				334.74		2.349215

				334.76		2.349215

				334.79		2.349215

				334.81		2.353614

				334.83		2.353614

				334.85		2.353614

				334.87		2.349215

				334.89		2.349215

				334.91		2.349215

				334.93		2.349215

				334.95		2.349215

				334.98		2.349215

				335		2.349215

				335.02		2.349215

				335.04		2.349215

				335.06		2.349215

				335.08		2.349215

				335.1		2.349215

				335.12		2.349215

				335.14		2.349215

				335.16		2.349215

				335.19		2.349215

				335.21		2.349215

				335.23		2.349215

				335.25		2.344815

				335.27		2.349215

				335.29		2.349215

				335.31		2.349215

				335.33		2.349215

				335.35		2.349215

				335.38		2.349215

				335.4		2.349215

				335.42		2.349215

				335.44		2.349215

				335.46		2.349215

				335.48		2.349215

				335.5		2.349215

				335.52		2.349215

				335.54		2.349215

				335.57		2.349215

				335.59		2.349215

				335.61		2.349215

				335.63		2.349215

				335.65		2.349215

				335.67		2.349215

				335.69		2.349215

				335.71		2.349215

				335.73		2.349215

				335.76		2.349215

				335.78		2.349215

				335.8		2.349215

				335.82		2.349215

				335.84		2.349215

				335.86		2.349215

				335.88		2.349215

				335.9		2.349215

				335.92		2.349215

				335.95		2.349215

				335.97		2.349215

				335.99		2.349215

				336.01		2.349215

				336.03		2.349215

				336.05		2.349215

				336.07		2.349215

				336.09		2.349215

				336.11		2.349215

				336.14		2.349215

				336.16		2.349215

				336.18		2.349215

				336.2		2.349215

				336.22		2.349215

				336.24		2.349215

				336.26		2.349215

				336.28		2.349215

				336.3		2.349215

				336.33		2.353614

				336.35		2.353614

				336.37		2.353614

				336.39		2.353614

				336.41		2.353614

				336.43		2.353614

				336.45		2.353614

				336.47		2.353614

				336.49		2.353614

				336.52		2.353614

				336.54		2.353614

				336.56		2.353614

				336.58		2.353614

				336.6		2.353614

				336.62		2.353614

				336.64		2.353614

				336.66		2.353614

				336.68		2.353614

				336.71		2.353614

				336.73		2.353614

				336.75		2.358013

				336.77		2.358013

				336.79		2.358013

				336.81		2.358013

				336.83		2.358013

				336.85		2.358013

				336.87		2.358013

				336.9		2.358013

				336.92		2.358013

				336.94		2.358013

				336.96		2.358013

				336.98		2.358013

				337		2.358013

				337.02		2.358013

				337.04		2.358013

				337.06		2.358013

				337.09		2.358013

				337.11		2.362413

				337.13		2.358013

				337.15		2.358013

				337.17		2.362413

				337.19		2.362413

				337.21		2.362413

				337.23		2.362413

				337.25		2.362413

				337.28		2.362413

				337.3		2.362413

				337.32		2.362413

				337.34		2.362413

				337.36		2.362413

				337.38		2.362413

				337.4		2.362413

				337.42		2.362413

				337.44		2.362413

				337.47		2.362413

				337.49		2.362413

				337.51		2.362413

				337.53		2.362413

				337.55		2.362413

				337.57		2.362413

				337.59		2.362413

				337.61		2.362413

				337.63		2.362413

				337.66		2.362413

				337.68		2.362413

				337.7		2.362413

				337.72		2.362413

				337.74		2.362413

				337.76		2.362413

				337.78		2.362413

				337.8		2.362413

				337.82		2.362413

				337.85		2.362413

				337.87		2.362413

				337.89		2.362413

				337.91		2.362413

				337.93		2.362413

				337.95		2.362413

				337.97		2.362413

				337.99		2.362413

				338.01		2.362413

				338.03		2.362413

				338.06		2.366812

				338.08		2.366812

				338.1		2.366812

				338.12		2.366812

				338.14		2.366812

				338.16		2.366812

				338.18		2.366812

				338.2		2.366812

				338.22		2.366812

				338.25		2.366812

				338.27		2.366812

				338.29		2.366812

				338.31		2.366812

				338.33		2.366812

				338.35		2.366812

				338.37		2.366812

				338.39		2.366812

				338.41		2.366812

				338.44		2.366812

				338.46		2.366812

				338.48		2.366812

				338.5		2.366812

				338.52		2.366812

				338.54		2.366812

				338.56		2.366812

				338.58		2.366812

				338.6		2.366812

				338.63		2.366812

				338.65		2.366812

				338.67		2.366812

				338.69		2.366812

				338.71		2.366812

				338.73		2.366812

				338.75		2.366812

				338.77		2.366812

				338.79		2.366812

				338.82		2.366812

				338.84		2.366812

				338.86		2.366812

				338.88		2.366812

				338.9		2.366812

				338.92		2.366812

				338.94		2.366812

				338.96		2.366812

				338.98		2.366812

				339.01		2.366812

				339.03		2.366812

				339.05		2.366812

				339.07		2.366812

				339.09		2.366812

				339.11		2.366812

				339.13		2.362413

				339.15		2.366812

				339.17		2.366812

				339.2		2.362413

				339.22		2.366812

				339.24		2.366812

				339.26		2.366812

				339.28		2.366812

				339.3		2.362413

				339.32		2.366812

				339.34		2.366812

				339.36		2.362413

				339.39		2.362413

				339.41		2.362413

				339.43		2.362413

				339.45		2.362413

				339.47		2.362413

				339.49		2.362413

				339.51		2.362413

				339.53		2.362413

				339.56		2.362413

				339.58		2.362413

				339.6		2.362413

				339.62		2.362413

				339.64		2.362413

				339.66		2.362413

				339.68		2.362413

				339.7		2.362413

				339.72		2.362413

				339.75		2.362413

				339.77		2.362413

				339.79		2.358013

				339.81		2.358013

				339.83		2.358013

				339.85		2.358013

				339.87		2.358013

				339.89		2.358013

				339.91		2.358013

				339.94		2.358013

				339.96		2.358013

				339.98		2.358013

				340		2.358013

				340.02		2.358013

				340.04		2.358013

				340.06		2.358013

				340.08		2.358013

				340.1		2.358013

				340.13		2.358013

				340.15		2.353614

				340.17		2.353614

				340.19		2.353614

				340.21		2.353614

				340.23		2.353614

				340.25		2.353614

				340.27		2.353614

				340.29		2.353614

				340.32		2.353614

				340.34		2.353614

				340.36		2.353614

				340.38		2.353614

				340.4		2.353614

				340.42		2.353614

				340.44		2.353614

				340.46		2.353614

				340.48		2.353614

				340.51		2.353614

				340.53		2.349215

				340.55		2.349215

				340.57		2.349215

				340.59		2.349215

				340.61		2.349215

				340.63		2.349215

				340.65		2.349215

				340.67		2.349215

				340.7		2.349215

				340.72		2.349215

				340.74		2.349215

				340.76		2.349215

				340.78		2.349215

				340.8		2.344815

				340.82		2.349215

				340.84		2.344815

				340.86		2.344815

				340.89		2.344815

				340.91		2.344815

				340.93		2.344815

				340.95		2.344815

				340.97		2.344815

				340.99		2.344815

				341.01		2.344815

				341.03		2.344815

				341.05		2.344815

				341.08		2.344815

				341.1		2.344815

				341.12		2.344815

				341.14		2.344815

				341.16		2.344815

				341.18		2.344815

				341.2		2.340416

				341.22		2.344815

				341.24		2.340416

				341.27		2.340416

				341.29		2.340416

				341.31		2.340416

				341.33		2.340416

				341.35		2.340416

				341.37		2.340416

				341.39		2.340416

				341.41		2.340416

				341.43		2.340416

				341.46		2.340416

				341.48		2.340416

				341.5		2.340416

				341.52		2.340416

				341.54		2.340416

				341.56		2.340416

				341.58		2.340416

				341.6		2.340416

				341.62		2.340416

				341.65		2.340416

				341.67		2.340416

				341.69		2.340416

				341.71		2.340416

				341.73		2.340416

				341.75		2.340416

				341.77		2.340416

				341.79		2.340416

				341.81		2.340416

				341.84		2.340416

				341.86		2.340416

				341.88		2.340416

				341.9		2.340416

				341.92		2.340416

				341.94		2.340416

				341.96		2.340416

				341.98		2.340416

				342		2.340416

				342.03		2.340416

				342.05		2.340416

				342.07		2.340416

				342.09		2.340416

				342.11		2.340416

				342.13		2.340416

				342.15		2.340416

				342.17		2.340416

				342.19		2.340416

				342.22		2.340416

				342.24		2.340416

				342.26		2.340416

				342.28		2.340416

				342.3		2.340416

				342.32		2.340416

				342.34		2.340416

				342.36		2.340416

				342.39		2.340416

				342.41		2.340416

				342.43		2.340416

				342.45		2.340416

				342.47		2.340416

				342.49		2.340416

				342.51		2.340416

				342.53		2.340416

				342.55		2.340416

				342.58		2.340416

				342.6		2.340416

				342.62		2.340416

				342.64		2.340416

				342.66		2.340416

				342.68		2.340416

				342.7		2.340416

				342.72		2.340416

				342.74		2.340416

				342.77		2.340416

				342.79		2.340416

				342.81		2.340416

				342.83		2.340416

				342.85		2.340416

				342.87		2.340416

				342.89		2.340416

				342.91		2.340416

				342.93		2.340416

				342.96		2.340416

				342.98		2.340416

				343		2.340416

				343.02		2.340416

				343.04		2.340416

				343.06		2.340416

				343.08		2.340416

				343.1		2.340416

				343.12		2.340416

				343.14		2.340416

				343.17		2.340416

				343.19		2.340416

				343.21		2.340416

				343.23		2.340416

				343.25		2.340416

				343.27		2.340416

				343.29		2.340416

				343.31		2.340416

				343.33		2.340416

				343.36		2.340416

				343.38		2.340416

				343.4		2.340416

				343.42		2.340416

				343.44		2.340416

				343.46		2.340416

				343.48		2.340416

				343.5		2.340416

				343.52		2.340416

				343.55		2.340416

				343.57		2.340416

				343.59		2.340416

				343.61		2.340416

				343.63		2.340416

				343.65		2.340416

				343.67		2.340416

				343.69		2.340416

				343.71		2.340416

				343.74		2.340416

				343.76		2.340416

				343.78		2.340416

				343.8		2.340416

				343.82		2.340416

				343.84		2.340416

				343.86		2.340416

				343.88		2.340416

				343.9		2.344815

				343.93		2.344815

				343.95		2.344815

				343.97		2.344815

				343.99		2.344815

				344.01		2.344815

				344.03		2.344815

				344.05		2.344815

				344.07		2.344815

				344.09		2.344815

				344.12		2.344815

				344.14		2.344815

				344.16		2.344815

				344.18		2.344815

				344.2		2.344815

				344.22		2.344815

				344.24		2.344815

				344.26		2.344815

				344.28		2.344815

				344.31		2.344815

				344.33		2.344815

				344.35		2.344815

				344.37		2.344815

				344.39		2.344815

				344.41		2.344815

				344.43		2.344815

				344.45		2.344815

				344.47		2.344815

				344.5		2.344815

				344.52		2.344815

				344.54		2.344815

				344.56		2.344815

				344.58		2.344815

				344.6		2.344815

				344.62		2.344815

				344.64		2.344815

				344.66		2.344815

				344.69		2.344815

				344.71		2.344815

				344.73		2.344815

				344.75		2.344815

				344.77		2.344815

				344.79		2.344815

				344.81		2.344815

				344.83		2.344815

				344.86		2.344815

				344.88		2.344815

				344.9		2.344815

				344.92		2.344815

				344.94		2.349215

				344.96		2.344815

				344.98		2.344815

				345		2.349215

				345.02		2.349215

				345.05		2.349215

				345.07		2.349215

				345.09		2.349215

				345.11		2.349215

				345.13		2.349215

				345.15		2.349215

				345.17		2.349215

				345.19		2.349215

				345.21		2.344815

				345.24		2.349215

				345.26		2.349215

				345.28		2.349215

				345.3		2.349215

				345.32		2.344815

				345.34		2.349215

				345.36		2.344815

				345.38		2.344815

				345.4		2.344815

				345.43		2.344815

				345.45		2.344815

				345.47		2.344815

				345.49		2.344815

				345.51		2.344815

				345.53		2.344815

				345.55		2.344815

				345.57		2.344815

				345.59		2.344815

				345.62		2.344815

				345.64		2.344815

				345.66		2.344815

				345.68		2.344815

				345.7		2.344815

				345.72		2.344815

				345.74		2.344815

				345.76		2.344815

				345.79		2.344815

				345.81		2.344815

				345.83		2.344815

				345.85		2.344815

				345.87		2.344815

				345.89		2.344815

				345.91		2.344815

				345.93		2.344815

				345.95		2.349215

				345.98		2.344815

				346		2.349215

				346.02		2.344815

				346.04		2.344815

				346.06		2.344815

				346.08		2.344815

				346.1		2.344815

				346.12		2.344815

				346.14		2.344815

				346.17		2.344815

				346.19		2.344815

				346.21		2.344815

				346.23		2.344815

				346.25		2.344815

				346.27		2.344815

				346.29		2.344815

				346.31		2.344815

				346.33		2.344815

				346.36		2.344815

				346.38		2.344815

				346.4		2.344815

				346.42		2.344815

				346.44		2.344815

				346.46		2.344815

				346.48		2.344815

				346.5		2.344815

				346.53		2.344815

				346.55		2.344815

				346.57		2.349215

				346.59		2.349215

				346.61		2.349215

				346.63		2.349215

				346.65		2.349215

				346.67		2.349215

				346.69		2.349215

				346.72		2.349215

				346.74		2.349215

				346.76		2.349215

				346.78		2.349215

				346.8		2.349215

				346.82		2.349215

				346.84		2.349215

				346.86		2.349215

				346.88		2.349215

				346.91		2.349215

				346.93		2.349215

				346.95		2.349215

				346.97		2.349215

				346.99		2.349215

				347.01		2.349215

				347.03		2.349215

				347.05		2.349215

				347.07		2.349215

				347.1		2.349215

				347.12		2.349215

				347.14		2.349215

				347.16		2.349215

				347.18		2.349215

				347.2		2.349215

				347.22		2.349215

				347.24		2.349215

				347.27		2.353614

				347.29		2.353614

				347.31		2.353614

				347.33		2.353614

				347.35		2.353614

				347.37		2.353614

				347.39		2.353614

				347.41		2.353614

				347.43		2.353614

				347.46		2.353614

				347.48		2.353614

				347.5		2.353614

				347.52		2.353614

				347.54		2.353614

				347.56		2.353614

				347.58		2.353614

				347.6		2.353614

				347.62		2.353614

				347.65		2.353614

				347.67		2.353614

				347.69		2.353614

				347.71		2.353614

				347.73		2.353614

				347.75		2.353614

				347.77		2.353614

				347.79		2.353614

				347.82		2.353614

				347.84		2.353614

				347.86		2.353614

				347.88		2.353614

				347.9		2.353614

				347.92		2.353614

				347.94		2.353614

				347.96		2.353614

				347.98		2.353614

				348.01		2.353614

				348.03		2.353614

				348.05		2.353614

				348.07		2.353614

				348.09		2.353614

				348.11		2.353614

				348.13		2.353614

				348.15		2.353614

				348.17		2.353614

				348.2		2.353614

				348.22		2.358013

				348.24		2.358013

				348.26		2.358013

				348.28		2.358013

				348.3		2.353614

				348.32		2.358013

				348.34		2.358013

				348.37		2.358013

				348.39		2.358013

				348.41		2.353614

				348.43		2.358013

				348.45		2.358013

				348.47		2.358013

				348.49		2.358013

				348.51		2.358013

				348.53		2.358013

				348.56		2.358013

				348.58		2.358013

				348.6		2.358013

				348.62		2.358013

				348.64		2.358013

				348.66		2.358013

				348.68		2.358013

				348.7		2.358013

				348.72		2.358013

				348.75		2.358013

				348.77		2.358013

				348.79		2.358013

				348.81		2.358013

				348.83		2.358013

				348.85		2.358013

				348.87		2.358013

				348.89		2.358013

				348.92		2.358013

				348.94		2.358013

				348.96		2.358013

				348.98		2.358013

				349		2.358013

				349.02		2.358013

				349.04		2.358013

				349.06		2.358013

				349.08		2.358013

				349.11		2.358013

				349.13		2.358013

				349.15		2.358013

				349.17		2.358013

				349.19		2.358013

				349.21		2.362413

				349.23		2.362413

				349.25		2.362413

				349.28		2.362413

				349.3		2.362413

				349.32		2.362413

				349.34		2.362413

				349.36		2.362413

				349.38		2.362413

				349.4		2.362413

				349.43		2.362413

				349.45		2.362413

				349.47		2.362413

				349.49		2.362413

				349.51		2.362413

				349.53		2.362413

				349.55		2.362413

				349.57		2.362413

				349.6		2.362413

				349.62		2.362413

				349.64		2.366812

				349.66		2.366812

				349.68		2.366812

				349.7		2.366812

				349.72		2.366812

				349.75		2.366812

				349.77		2.366812

				349.79		2.366812

				349.81		2.366812

				349.83		2.366812

				349.85		2.366812

				349.87		2.366812

				349.9		2.366812

				349.92		2.366812

				349.94		2.366812

				349.96		2.366812

				349.98		2.366812

				350		2.366812

				350.02		2.366812

				350.05		2.366812

				350.07		2.366812

				350.09		2.366812

				350.11		2.366812

				350.13		2.366812

				350.15		2.366812

				350.17		2.366812

				350.19		2.366812

				350.22		2.366812

				350.24		2.366812

				350.26		2.366812

				350.28		2.366812

				350.3		2.366812

				350.32		2.366812

				350.34		2.366812

				350.37		2.366812

				350.39		2.371211

				350.41		2.371211

				350.43		2.371211

				350.45		2.371211

				350.47		2.371211

				350.49		2.371211

				350.51		2.371211

				350.53		2.371211

				350.56		2.371211

				350.58		2.371211

				350.6		2.371211

				350.62		2.371211

				350.64		2.371211

				350.66		2.371211

				350.68		2.371211

				350.7		2.371211

				350.73		2.371211

				350.75		2.371211

				350.77		2.371211

				350.79		2.371211

				350.81		2.371211

				350.83		2.371211

				350.85		2.366812

				350.87		2.366812

				350.9		2.366812

				350.92		2.366812

				350.94		2.366812

				350.96		2.366812

				350.98		2.366812

				351		2.366812

				351.02		2.366812

				351.04		2.366812

				351.06		2.366812

				351.09		2.366812

				351.11		2.366812

				351.13		2.366812

				351.15		2.366812

				351.17		2.366812

				351.19		2.366812

				351.21		2.366812

				351.23		2.366812

				351.26		2.366812

				351.28		2.366812

				351.3		2.366812

				351.32		2.366812

				351.34		2.366812

				351.36		2.366812

				351.38		2.366812

				351.4		2.366812

				351.43		2.366812

				351.45		2.366812

				351.47		2.366812

				351.49		2.366812

				351.51		2.366812

				351.53		2.366812

				351.55		2.366812

				351.57		2.366812

				351.6		2.366812

				351.62		2.366812

				351.64		2.366812

				351.66		2.366812

				351.68		2.366812

				351.7		2.362413

				351.72		2.362413

				351.74		2.362413

				351.77		2.362413

				351.79		2.366812

				351.81		2.362413

				351.83		2.362413

				351.85		2.362413

				351.87		2.362413

				351.89		2.362413

				351.91		2.362413

				351.94		2.362413

				351.96		2.362413

				351.98		2.362413

				352		2.362413

				352.02		2.362413

				352.04		2.362413

				352.06		2.362413

				352.08		2.362413

				352.11		2.362413

				352.13		2.362413

				352.15		2.362413

				352.17		2.362413

				352.19		2.362413

				352.21		2.362413

				352.23		2.362413

				352.25		2.362413

				352.28		2.362413

				352.3		2.362413

				352.32		2.362413

				352.34		2.362413

				352.36		2.358013

				352.38		2.362413

				352.4		2.358013

				352.42		2.358013

				352.45		2.358013

				352.47		2.358013

				352.49		2.358013

				352.51		2.358013

				352.53		2.358013

				352.55		2.358013

				352.57		2.358013

				352.59		2.358013

				352.62		2.358013

				352.64		2.358013

				352.66		2.358013

				352.68		2.358013

				352.7		2.358013

				352.72		2.358013

				352.74		2.358013

				352.76		2.358013

				352.79		2.358013

				352.81		2.353614

				352.83		2.353614

				352.85		2.353614

				352.87		2.353614

				352.89		2.353614

				352.91		2.353614

				352.93		2.353614

				352.95		2.353614

				352.98		2.353614

				353		2.353614

				353.02		2.353614

				353.04		2.353614

				353.06		2.353614

				353.08		2.353614

				353.1		2.353614

				353.12		2.353614

				353.15		2.353614

				353.17		2.353614

				353.19		2.353614

				353.21		2.353614

				353.23		2.353614

				353.25		2.353614

				353.27		2.353614

				353.29		2.349215

				353.32		2.349215

				353.34		2.349215

				353.36		2.349215

				353.38		2.349215

				353.4		2.349215

				353.42		2.349215

				353.44		2.349215

				353.46		2.349215

				353.49		2.349215

				353.51		2.349215

				353.53		2.349215

				353.55		2.349215

				353.57		2.349215

				353.59		2.349215

				353.61		2.349215

				353.63		2.349215

				353.66		2.349215

				353.68		2.349215

				353.7		2.349215

				353.72		2.349215

				353.74		2.349215

				353.76		2.349215

				353.78		2.349215

				353.8		2.349215

				353.83		2.349215

				353.85		2.349215

				353.87		2.349215

				353.89		2.349215

				353.91		2.349215

				353.93		2.349215

				353.95		2.349215

				353.97		2.349215

				354		2.349215

				354.02		2.344815

				354.04		2.344815

				354.06		2.344815

				354.08		2.344815

				354.1		2.344815

				354.12		2.344815

				354.15		2.344815

				354.17		2.344815

				354.19		2.344815

				354.21		2.344815

				354.23		2.344815

				354.25		2.344815

				354.27		2.344815

				354.29		2.344815

				354.32		2.344815

				354.34		2.344815

				354.36		2.344815

				354.38		2.344815

				354.4		2.344815

				354.42		2.344815

				354.44		2.344815

				354.46		2.344815

				354.49		2.344815

				354.51		2.344815

				354.53		2.344815

				354.55		2.344815

				354.57		2.344815

				354.59		2.344815

				354.61		2.344815

				354.63		2.344815

				354.66		2.344815

				354.68		2.344815

				354.7		2.344815

				354.72		2.344815

				354.74		2.344815

				354.76		2.344815

				354.78		2.344815

				354.8		2.344815

				354.83		2.344815

				354.85		2.344815

				354.87		2.344815

				354.89		2.344815

				354.91		2.344815

				354.93		2.344815

				354.95		2.344815

				354.98		2.349215

				355		2.344815

				355.02		2.344815

				355.04		2.349215

				355.06		2.344815

				355.08		2.344815

				355.1		2.344815

				355.12		2.344815

				355.15		2.344815

				355.17		2.344815

				355.19		2.344815

				355.21		2.344815

				355.23		2.344815

				355.25		2.344815

				355.27		2.344815

				355.29		2.344815

				355.32		2.344815

				355.34		2.349215

				355.36		2.349215

				355.38		2.349215

				355.4		2.349215

				355.42		2.349215

				355.44		2.349215

				355.46		2.349215

				355.49		2.349215

				355.51		2.349215

				355.53		2.349215

				355.55		2.349215

				355.57		2.349215

				355.59		2.349215

				355.61		2.349215

				355.63		2.349215

				355.66		2.349215

				355.68		2.349215

				355.7		2.353614

				355.72		2.349215

				355.74		2.349215

				355.76		2.353614

				355.78		2.353614

				355.8		2.349215

				355.83		2.353614

				355.85		2.353614

				355.87		2.353614

				355.89		2.353614

				355.91		2.353614

				355.93		2.353614

				355.95		2.353614

				355.97		2.353614

				356		2.353614

				356.02		2.353614

				356.04		2.353614

				356.06		2.353614

				356.08		2.353614

				356.1		2.353614

				356.12		2.353614

				356.14		2.353614

				356.17		2.353614

				356.19		2.353614

				356.21		2.353614

				356.23		2.353614

				356.25		2.353614

				356.27		2.353614

				356.29		2.353614

				356.31		2.353614

				356.34		2.353614

				356.36		2.353614

				356.38		2.358013

				356.4		2.358013

				356.42		2.358013

				356.44		2.358013

				356.46		2.358013

				356.48		2.358013

				356.51		2.358013

				356.53		2.358013

				356.55		2.358013

				356.57		2.358013

				356.59		2.358013

				356.61		2.358013

				356.63		2.358013

				356.65		2.358013

				356.68		2.358013

				356.7		2.358013

				356.72		2.358013

				356.74		2.358013

				356.76		2.358013

				356.78		2.358013

				356.8		2.358013

				356.82		2.358013

				356.85		2.358013

				356.87		2.358013

				356.89		2.358013

				356.91		2.358013

				356.93		2.358013

				356.95		2.358013

				356.97		2.358013

				356.99		2.358013

				357.02		2.358013

				357.04		2.358013

				357.06		2.358013

				357.08		2.358013

				357.1		2.358013

				357.12		2.358013

				357.14		2.358013

				357.16		2.358013

				357.19		2.358013

				357.21		2.358013

				357.23		2.358013

				357.25		2.358013

				357.27		2.358013

				357.29		2.358013

				357.31		2.358013

				357.33		2.358013

				357.35		2.358013

				357.38		2.358013

				357.4		2.358013

				357.42		2.358013

				357.44		2.358013

				357.46		2.358013

				357.48		2.358013

				357.5		2.358013

				357.52		2.358013

				357.55		2.358013

				357.57		2.358013

				357.59		2.358013

				357.61		2.358013

				357.63		2.358013

				357.65		2.353614

				357.67		2.358013

				357.69		2.353614

				357.72		2.353614

				357.74		2.353614

				357.76		2.353614

				357.78		2.353614

				357.8		2.353614

				357.82		2.353614

				357.84		2.353614

				357.86		2.353614

				357.88		2.353614

				357.91		2.353614

				357.93		2.353614

				357.95		2.353614

				357.97		2.353614

				357.99		2.353614

				358.01		2.353614

				358.03		2.353614

				358.05		2.353614

				358.08		2.353614

				358.1		2.353614

				358.12		2.353614

				358.14		2.353614

				358.16		2.353614

				358.18		2.353614

				358.2		2.353614

				358.22		2.353614

				358.25		2.353614

				358.27		2.353614

				358.29		2.353614

				358.31		2.353614

				358.33		2.353614

				358.35		2.353614

				358.37		2.353614

				358.39		2.353614

				358.41		2.353614

				358.44		2.353614

				358.46		2.353614

				358.48		2.353614

				358.5		2.353614

				358.52		2.353614

				358.54		2.353614

				358.56		2.353614

				358.58		2.353614

				358.61		2.353614

				358.63		2.353614

				358.65		2.353614

				358.67		2.353614

				358.69		2.353614

				358.71		2.353614

				358.73		2.353614

				358.75		2.353614

				358.78		2.353614

				358.8		2.353614

				358.82		2.353614

				358.84		2.353614

				358.86		2.353614

				358.88		2.353614

				358.9		2.353614

				358.92		2.353614

				358.94		2.353614

				358.97		2.353614

				358.99		2.353614

				359.01		2.353614

				359.03		2.353614

				359.05		2.353614

				359.07		2.353614

				359.09		2.353614

				359.11		2.353614

				359.14		2.353614

				359.16		2.353614

				359.18		2.353614

				359.2		2.353614

				359.22		2.353614

				359.24		2.353614

				359.26		2.353614

				359.28		2.353614

				359.31		2.353614

				359.33		2.353614

				359.35		2.353614

				359.37		2.353614

				359.39		2.353614

				359.41		2.353614

				359.43		2.353614

				359.45		2.353614

				359.48		2.353614

				359.5		2.353614

				359.52		2.353614

				359.54		2.353614

				359.56		2.353614

				359.58		2.353614

				359.6		2.353614

				359.62		2.353614

				359.65		2.353614

				359.67		2.353614

				359.69		2.353614

				359.71		2.353614

				359.73		2.353614

				359.75		2.353614

				359.77		2.353614

				359.79		2.353614

				359.81		2.353614

				359.84		2.353614

				359.86		2.353614

				359.88		2.353614

				359.9		2.353614

				359.92		2.353614

				359.94		2.353614

				359.96		2.353614

				359.98		2.353614

				360.01		2.353614

				360.03		2.353614

				360.05		2.353614

				360.07		2.353614

				360.09		2.353614

				360.11		2.353614

				360.13		2.353614

				360.15		2.353614

				360.18		2.353614

				360.2		2.353614

				360.22		2.353614

				360.24		2.353614

				360.26		2.353614

				360.28		2.353614

				360.3		2.353614

				360.32		2.353614

				360.35		2.353614

				360.37		2.353614

				360.39		2.353614

				360.41		2.353614

				360.43		2.353614

				360.45		2.353614

				360.47		2.353614

				360.49		2.353614

				360.52		2.353614

				360.54		2.353614

				360.56		2.353614

				360.58		2.353614

				360.6		2.353614

				360.62		2.353614

				360.64		2.353614

				360.66		2.353614

				360.68		2.353614

				360.71		2.353614

				360.73		2.353614

				360.75		2.353614

				360.77		2.353614

				360.79		2.353614

				360.81		2.353614

				360.83		2.353614

				360.85		2.353614

				360.88		2.353614

				360.9		2.353614

				360.92		2.353614

				360.94		2.353614

				360.96		2.353614

				360.98		2.353614

				361		2.353614

				361.02		2.353614

				361.05		2.353614

				361.07		2.353614

				361.09		2.353614

				361.11		2.353614

				361.13		2.353614

				361.15		2.353614

				361.17		2.353614

				361.19		2.353614

				361.21		2.353614

				361.24		2.353614

				361.26		2.353614

				361.28		2.353614

				361.3		2.353614

				361.32		2.353614

				361.34		2.353614

				361.36		2.353614

				361.38		2.353614

				361.41		2.353614

				361.43		2.353614

				361.45		2.353614

				361.47		2.353614

				361.49		2.353614

				361.51		2.353614

				361.53		2.353614

				361.55		2.353614

				361.58		2.353614

				361.6		2.353614

				361.62		2.353614

				361.64		2.353614

				361.66		2.353614

				361.68		2.353614

				361.7		2.353614

				361.72		2.353614

				361.75		2.358013

				361.77		2.353614

				361.79		2.358013

				361.81		2.353614

				361.83		2.358013

				361.85		2.358013

				361.87		2.358013

				361.89		2.358013

				361.92		2.358013

				361.94		2.353614

				361.96		2.353614

				361.98		2.353614

				362		2.353614

				362.02		2.358013

				362.04		2.358013

				362.06		2.358013

				362.08		2.358013

				362.11		2.358013

				362.13		2.358013

				362.15		2.358013

				362.17		2.358013

				362.19		2.358013

				362.21		2.358013

				362.23		2.358013

				362.25		2.358013

				362.28		2.358013

				362.3		2.358013

				362.32		2.358013

				362.34		2.358013

				362.36		2.358013

				362.38		2.358013

				362.4		2.358013

				362.42		2.358013

				362.45		2.358013

				362.47		2.358013

				362.49		2.358013

				362.51		2.358013

				362.53		2.358013

				362.55		2.358013

				362.57		2.358013

				362.59		2.358013

				362.62		2.358013

				362.64		2.358013

				362.66		2.358013

				362.68		2.358013

				362.7		2.358013

				362.72		2.358013

				362.74		2.358013

				362.76		2.358013

				362.78		2.358013

				362.81		2.358013

				362.83		2.358013

				362.85		2.358013

				362.87		2.358013

				362.89		2.358013

				362.91		2.358013

				362.93		2.358013

				362.95		2.358013

				362.98		2.358013

				363		2.358013

				363.02		2.358013

				363.04		2.358013

				363.06		2.358013

				363.08		2.358013

				363.1		2.358013

				363.12		2.358013

				363.15		2.358013

				363.17		2.358013

				363.19		2.358013

				363.21		2.358013

				363.23		2.358013

				363.25		2.358013

				363.27		2.358013

				363.29		2.358013

				363.32		2.358013

				363.34		2.358013

				363.36		2.358013

				363.38		2.358013

				363.4		2.358013

				363.42		2.358013

				363.44		2.358013

				363.46		2.358013

				363.49		2.358013

				363.51		2.358013

				363.53		2.358013

				363.55		2.358013

				363.57		2.358013

				363.59		2.358013

				363.61		2.358013

				363.63		2.358013

				363.66		2.358013

				363.68		2.358013

				363.7		2.358013

				363.72		2.358013

				363.74		2.358013

				363.76		2.358013

				363.78		2.358013

				363.8		2.358013

				363.83		2.353614

				363.85		2.353614

				363.87		2.353614

				363.89		2.353614

				363.91		2.353614

				363.93		2.353614

				363.95		2.353614

				363.97		2.353614

				363.99		2.353614

				364.02		2.353614

				364.04		2.353614

				364.06		2.353614

				364.08		2.353614

				364.1		2.353614

				364.12		2.353614

				364.14		2.353614

				364.16		2.353614

				364.19		2.353614

				364.21		2.353614

				364.23		2.353614

				364.25		2.353614

				364.27		2.353614

				364.29		2.353614

				364.31		2.353614

				364.33		2.353614

				364.36		2.353614

				364.38		2.353614

				364.4		2.353614

				364.42		2.353614

				364.44		2.353614

				364.46		2.353614

				364.48		2.353614

				364.5		2.353614

				364.53		2.353614

				364.55		2.353614

				364.57		2.353614

				364.59		2.353614

				364.61		2.353614

				364.63		2.353614

				364.65		2.353614

				364.67		2.353614

				364.69		2.353614

				364.72		2.353614

				364.74		2.353614

				364.76		2.358013

				364.78		2.353614

				364.8		2.358013

				364.82		2.358013

				364.84		2.358013

				364.86		2.358013

				364.89		2.358013

				364.91		2.358013

				364.93		2.358013

				364.95		2.358013

				364.97		2.358013

				364.99		2.358013

				365.01		2.358013

				365.03		2.358013

				365.05		2.358013

				365.08		2.358013

				365.1		2.358013

				365.12		2.358013

				365.14		2.358013

				365.16		2.358013

				365.18		2.358013

				365.2		2.358013

				365.22		2.358013

				365.25		2.358013

				365.27		2.358013

				365.29		2.358013

				365.31		2.358013

				365.33		2.358013

				365.35		2.358013

				365.37		2.358013

				365.39		2.358013

				365.41		2.358013

				365.44		2.358013

				365.46		2.358013

				365.48		2.358013

				365.5		2.358013

				365.52		2.358013

				365.54		2.358013

				365.56		2.358013

				365.58		2.358013

				365.61		2.358013

				365.63		2.358013

				365.65		2.358013

				365.67		2.358013

				365.69		2.358013

				365.71		2.358013

				365.73		2.358013

				365.75		2.358013

				365.78		2.358013

				365.8		2.358013

				365.82		2.358013

				365.84		2.358013

				365.86		2.358013

				365.88		2.362413

				365.9		2.358013

				365.92		2.362413

				365.94		2.362413

				365.97		2.362413

				365.99		2.358013

				366.01		2.358013

				366.03		2.358013

				366.05		2.362413

				366.07		2.362413

				366.09		2.358013

				366.11		2.358013

				366.14		2.362413

				366.16		2.358013

				366.18		2.362413

				366.2		2.362413

				366.22		2.362413

				366.24		2.358013

				366.26		2.358013

				366.28		2.358013

				366.31		2.358013

				366.33		2.358013

				366.35		2.358013

				366.37		2.358013

				366.39		2.358013

				366.41		2.358013

				366.43		2.358013

				366.45		2.358013

				366.47		2.358013

				366.5		2.358013

				366.52		2.358013

				366.54		2.358013

				366.56		2.358013

				366.58		2.358013

				366.6		2.358013

				366.62		2.358013

				366.64		2.358013

				366.67		2.358013

				366.69		2.358013

				366.71		2.358013

				366.73		2.358013

				366.75		2.358013

				366.77		2.358013

				366.79		2.358013

				366.81		2.358013

				366.84		2.358013

				366.86		2.358013

				366.88		2.358013

				366.9		2.358013

				366.92		2.358013

				366.94		2.358013

				366.96		2.358013

				366.98		2.358013

				367.01		2.358013

				367.03		2.358013

				367.05		2.358013

				367.07		2.358013

				367.09		2.358013

				367.11		2.358013

				367.13		2.358013

				367.15		2.358013

				367.17		2.358013

				367.2		2.358013

				367.22		2.358013

				367.24		2.358013

				367.26		2.358013

				367.28		2.358013

				367.3		2.358013

				367.32		2.358013

				367.34		2.358013

				367.37		2.353614

				367.39		2.353614

				367.41		2.353614

				367.43		2.353614

				367.45		2.353614

				367.47		2.353614

				367.49		2.353614

				367.51		2.353614

				367.54		2.353614

				367.56		2.353614

				367.58		2.353614

				367.6		2.353614

				367.62		2.353614

				367.64		2.353614

				367.66		2.353614

				367.68		2.353614

				367.71		2.353614

				367.73		2.353614

				367.75		2.353614

				367.77		2.353614

				367.79		2.353614

				367.81		2.353614

				367.83		2.353614

				367.85		2.353614

				367.88		2.353614

				367.9		2.353614

				367.92		2.353614

				367.94		2.353614

				367.96		2.349215

				367.98		2.349215

				368		2.353614

				368.02		2.353614

				368.04		2.353614

				368.07		2.353614

				368.09		2.353614

				368.11		2.353614

				368.13		2.353614

				368.15		2.353614

				368.17		2.353614

				368.19		2.353614

				368.21		2.353614

				368.24		2.353614

				368.26		2.353614

				368.28		2.353614

				368.3		2.353614

				368.32		2.353614

				368.34		2.353614

				368.36		2.353614

				368.38		2.353614

				368.41		2.353614

				368.43		2.353614

				368.45		2.353614

				368.47		2.353614

				368.49		2.353614

				368.51		2.353614

				368.53		2.353614

				368.55		2.353614

				368.58		2.353614

				368.6		2.353614

				368.62		2.353614

				368.64		2.353614

				368.66		2.353614

				368.68		2.353614

				368.7		2.353614

				368.72		2.353614

				368.74		2.353614

				368.77		2.353614

				368.79		2.353614

				368.81		2.353614

				368.83		2.353614

				368.85		2.353614

				368.87		2.353614

				368.89		2.353614

				368.91		2.358013

				368.94		2.358013

				368.96		2.358013

				368.98		2.353614

				369		2.353614

				369.02		2.353614

				369.04		2.358013

				369.06		2.353614

				369.08		2.353614

				369.11		2.353614

				369.13		2.353614

				369.15		2.353614

				369.17		2.353614

				369.19		2.353614

				369.21		2.353614

				369.23		2.353614

				369.25		2.353614

				369.28		2.353614

				369.3		2.353614

				369.32		2.353614

				369.34		2.353614

				369.36		2.353614

				369.38		2.353614

				369.4		2.353614

				369.42		2.353614

				369.45		2.353614

				369.47		2.358013

				369.49		2.358013

				369.51		2.358013

				369.53		2.358013

				369.55		2.358013

				369.57		2.358013

				369.59		2.358013

				369.61		2.358013

				369.64		2.358013

				369.66		2.358013

				369.68		2.358013

				369.7		2.358013

				369.72		2.358013

				369.74		2.358013

				369.76		2.358013

				369.78		2.358013

				369.81		2.358013

				369.83		2.358013

				369.85		2.358013

				369.87		2.358013

				369.89		2.362413

				369.91		2.358013

				369.93		2.362413

				369.95		2.362413

				369.98		2.362413

				370		2.362413

				370.02		2.362413

				370.04		2.362413

				370.06		2.362413

				370.08		2.362413

				370.1		2.362413

				370.12		2.362413

				370.15		2.362413

				370.17		2.362413

				370.19		2.362413

				370.21		2.362413

				370.23		2.362413

				370.25		2.362413

				370.27		2.362413

				370.29		2.362413

				370.32		2.362413

				370.34		2.362413

				370.36		2.362413

				370.38		2.362413

				370.4		2.362413

				370.42		2.362413

				370.44		2.362413

				370.46		2.362413

				370.49		2.362413

				370.51		2.362413

				370.53		2.362413

				370.55		2.362413

				370.57		2.362413

				370.59		2.362413

				370.61		2.362413

				370.63		2.366812

				370.65		2.366812

				370.68		2.366812

				370.7		2.366812

				370.72		2.366812

				370.74		2.366812

				370.76		2.366812

				370.78		2.366812

				370.8		2.366812

				370.82		2.366812

				370.85		2.366812

				370.87		2.366812

				370.89		2.366812

				370.91		2.366812

				370.93		2.366812

				370.95		2.366812

				370.97		2.366812

				370.99		2.366812

				371.02		2.366812

				371.04		2.366812

				371.06		2.366812

				371.08		2.366812

				371.1		2.366812

				371.12		2.366812

				371.14		2.366812

				371.16		2.366812

				371.19		2.366812

				371.21		2.366812

				371.23		2.366812

				371.25		2.366812

				371.27		2.366812

				371.29		2.366812

				371.31		2.366812

				371.33		2.366812

				371.36		2.366812

				371.38		2.366812

				371.4		2.366812

				371.42		2.371211

				371.44		2.371211

				371.46		2.366812

				371.48		2.366812

				371.5		2.371211

				371.53		2.371211

				371.55		2.371211

				371.57		2.371211

				371.59		2.371211

				371.61		2.371211

				371.63		2.371211

				371.65		2.371211

				371.67		2.371211

				371.69		2.371211

				371.72		2.371211

				371.74		2.371211

				371.76		2.371211

				371.78		2.371211

				371.8		2.371211

				371.82		2.371211

				371.84		2.371211

				371.86		2.371211

				371.89		2.371211

				371.91		2.371211

				371.93		2.371211

				371.95		2.371211

				371.97		2.371211

				371.99		2.371211

				372.01		2.371211

				372.03		2.371211

				372.06		2.371211

				372.08		2.371211

				372.1		2.371211

				372.12		2.371211

				372.14		2.371211

				372.16		2.371211

				372.18		2.371211

				372.2		2.371211

				372.23		2.371211

				372.25		2.371211

				372.27		2.371211

				372.29		2.371211

				372.31		2.371211

				372.33		2.371211

				372.35		2.371211

				372.37		2.371211

				372.4		2.371211

				372.42		2.371211

				372.44		2.371211

				372.46		2.371211

				372.48		2.371211

				372.5		2.371211

				372.52		2.371211

				372.54		2.371211

				372.57		2.371211

				372.59		2.371211

				372.61		2.371211

				372.63		2.371211

				372.65		2.371211

				372.67		2.371211

				372.69		2.371211

				372.71		2.371211

				372.74		2.371211

				372.76		2.371211

				372.78		2.371211

				372.8		2.371211

				372.82		2.366812

				372.84		2.366812

				372.86		2.366812

				372.88		2.366812

				372.91		2.366812

				372.93		2.366812

				372.95		2.366812

				372.97		2.366812

				372.99		2.366812

				373.01		2.366812

				373.03		2.366812

				373.05		2.366812

				373.08		2.366812

				373.1		2.366812

				373.12		2.366812

				373.14		2.366812

				373.16		2.366812

				373.18		2.366812

				373.2		2.366812

				373.22		2.366812

				373.25		2.366812

				373.27		2.366812

				373.29		2.366812

				373.31		2.366812

				373.33		2.366812

				373.35		2.366812

				373.37		2.366812

				373.39		2.366812

				373.42		2.366812

				373.44		2.366812

				373.46		2.366812

				373.48		2.366812

				373.5		2.366812

				373.52		2.366812

				373.54		2.366812

				373.56		2.366812

				373.59		2.366812

				373.61		2.366812

				373.63		2.366812

				373.65		2.366812

				373.67		2.366812

				373.69		2.366812

				373.71		2.362413

				373.73		2.362413

				373.76		2.362413

				373.78		2.362413

				373.8		2.362413

				373.82		2.362413

				373.84		2.362413

				373.86		2.362413

				373.88		2.362413

				373.9		2.362413

				373.93		2.362413

				373.95		2.362413

				373.97		2.362413

				373.99		2.362413

				374.01		2.362413

				374.03		2.362413

				374.05		2.362413

				374.07		2.362413

				374.1		2.362413

				374.12		2.358013

				374.14		2.358013

				374.16		2.358013

				374.18		2.358013

				374.2		2.358013

				374.22		2.358013

				374.24		2.358013

				374.27		2.358013

				374.29		2.358013

				374.31		2.358013

				374.33		2.358013

				374.35		2.358013

				374.37		2.358013

				374.39		2.358013

				374.41		2.358013

				374.44		2.358013

				374.46		2.358013

				374.48		2.358013

				374.5		2.362413

				374.52		2.362413

				374.54		2.362413

				374.56		2.362413

				374.58		2.362413

				374.61		2.362413

				374.63		2.362413

				374.65		2.362413

				374.67		2.362413

				374.69		2.362413

				374.71		2.362413

				374.73		2.362413

				374.75		2.362413

				374.78		2.362413

				374.8		2.362413

				374.82		2.362413

				374.84		2.362413

				374.86		2.362413

				374.88		2.362413

				374.9		2.362413

				374.92		2.366812

				374.94		2.366812

				374.97		2.366812

				374.99		2.366812

				375.01		2.366812

				375.03		2.366812

				375.05		2.366812

				375.07		2.366812

				375.09		2.366812

				375.11		2.366812

				375.14		2.366812

				375.16		2.366812

				375.18		2.366812

				375.2		2.366812

				375.22		2.366812

				375.24		2.366812

				375.26		2.366812

				375.28		2.366812

				375.31		2.366812

				375.33		2.366812

				375.35		2.366812

				375.37		2.366812

				375.39		2.366812

				375.41		2.366812

				375.43		2.366812

				375.45		2.366812

				375.48		2.366812

				375.5		2.366812

				375.52		2.366812

				375.54		2.366812

				375.56		2.371211

				375.58		2.371211

				375.6		2.371211

				375.62		2.371211

				375.65		2.371211

				375.67		2.371211

				375.69		2.371211

				375.71		2.371211

				375.73		2.371211

				375.75		2.371211

				375.77		2.371211

				375.79		2.371211

				375.82		2.371211

				375.84		2.371211

				375.86		2.371211

				375.88		2.371211

				375.9		2.37561

				375.92		2.37561

				375.94		2.37561

				375.96		2.37561

				375.99		2.37561

				376.01		2.37561

				376.03		2.37561

				376.05		2.37561

				376.07		2.37561

				376.09		2.37561

				376.11		2.38001

				376.13		2.38001

				376.16		2.38001

				376.18		2.38001

				376.2		2.38001

				376.22		2.38001

				376.24		2.38001

				376.26		2.38001

				376.28		2.38001

				376.3		2.38001

				376.33		2.38001

				376.35		2.38001

				376.37		2.38001

				376.39		2.38001

				376.41		2.38001

				376.43		2.38001

				376.45		2.38001

				376.47		2.38001

				376.5		2.38001

				376.52		2.38001

				376.54		2.38001

				376.56		2.38001

				376.58		2.38001

				376.6		2.38001

				376.62		2.38001

				376.64		2.38001

				376.67		2.384409

				376.69		2.384409

				376.71		2.384409

				376.73		2.384409

				376.75		2.384409

				376.77		2.384409

				376.79		2.384409

				376.81		2.384409

				376.84		2.384409

				376.86		2.384409

				376.88		2.384409

				376.9		2.384409

				376.92		2.384409

				376.94		2.384409

				376.96		2.384409

				376.98		2.384409

				377.01		2.384409

				377.03		2.38001

				377.05		2.38001

				377.07		2.384409

				377.09		2.384409

				377.11		2.384409

				377.13		2.384409

				377.15		2.38001

				377.18		2.384409

				377.2		2.384409

				377.22		2.384409

				377.24		2.384409

				377.26		2.384409

				377.28		2.384409

				377.3		2.384409

				377.32		2.384409

				377.35		2.384409

				377.37		2.384409

				377.39		2.384409

				377.41		2.384409

				377.43		2.384409

				377.45		2.384409

				377.47		2.384409

				377.49		2.384409

				377.52		2.384409

				377.54		2.384409

				377.56		2.384409

				377.58		2.384409

				377.6		2.384409

				377.62		2.384409

				377.64		2.384409

				377.66		2.384409

				377.68		2.384409

				377.71		2.384409

				377.73		2.384409

				377.75		2.384409

				377.77		2.384409

				377.79		2.38001

				377.81		2.384409

				377.83		2.384409

				377.85		2.384409

				377.88		2.38001

				377.9		2.38001

				377.92		2.38001

				377.94		2.38001

				377.96		2.38001

				377.98		2.38001

				378		2.38001

				378.02		2.38001

				378.05		2.38001

				378.07		2.38001

				378.09		2.38001

				378.11		2.38001

				378.13		2.38001

				378.15		2.38001

				378.17		2.38001

				378.19		2.38001

				378.22		2.38001

				378.24		2.38001

				378.26		2.38001

				378.28		2.38001

				378.3		2.38001

				378.32		2.38001

				378.34		2.38001

				378.36		2.38001

				378.39		2.38001

				378.41		2.38001

				378.43		2.38001

				378.45		2.38001

				378.47		2.38001

				378.49		2.38001

				378.51		2.38001

				378.53		2.38001

				378.56		2.38001

				378.58		2.38001

				378.6		2.38001

				378.62		2.38001

				378.64		2.38001

				378.66		2.38001

				378.68		2.38001

				378.7		2.38001

				378.73		2.38001

				378.75		2.38001

				378.77		2.38001

				378.79		2.38001

				378.81		2.38001

				378.83		2.38001

				378.85		2.38001

				378.87		2.38001

				378.9		2.38001

				378.92		2.38001

				378.94		2.38001

				378.96		2.38001

				378.98		2.38001

				379		2.38001

				379.02		2.38001

				379.04		2.38001

				379.07		2.38001

				379.09		2.384409

				379.11		2.38001

				379.13		2.384409

				379.15		2.384409

				379.17		2.38001

				379.19		2.38001

				379.21		2.384409

				379.24		2.384409

				379.26		2.384409

				379.28		2.384409

				379.3		2.384409

				379.32		2.384409

				379.34		2.384409

				379.36		2.384409

				379.38		2.384409

				379.41		2.384409

				379.43		2.384409

				379.45		2.384409

				379.47		2.384409

				379.49		2.384409

				379.51		2.384409

				379.53		2.384409

				379.55		2.384409

				379.58		2.384409

				379.6		2.384409

				379.62		2.384409

				379.64		2.384409

				379.66		2.384409

				379.68		2.388808

				379.7		2.388808

				379.72		2.388808

				379.74		2.388808

				379.77		2.388808

				379.79		2.388808

				379.81		2.388808

				379.83		2.388808

				379.85		2.388808

				379.87		2.388808

				379.89		2.388808

				379.91		2.388808

				379.94		2.388808

				379.96		2.388808

				379.98		2.388808

				380		2.393208

				380.02		2.393208

				380.04		2.393208

				380.06		2.393208

				380.08		2.393208

				380.11		2.393208

				380.13		2.393208

				380.15		2.393208

				380.17		2.393208

				380.19		2.393208

				380.21		2.393208

				380.23		2.393208

				380.25		2.393208

				380.28		2.393208

				380.3		2.393208

				380.32		2.393208

				380.34		2.393208

				380.36		2.393208

				380.38		2.393208

				380.4		2.393208

				380.42		2.393208

				380.45		2.393208

				380.47		2.393208

				380.49		2.393208

				380.51		2.393208

				380.53		2.397607

				380.55		2.397607

				380.57		2.397607

				380.59		2.397607

				380.62		2.397607

				380.64		2.397607

				380.66		2.397607

				380.68		2.397607

				380.7		2.397607

				380.72		2.397607

				380.74		2.397607

				380.76		2.397607

				380.78		2.397607

				380.81		2.397607

				380.83		2.397607

				380.85		2.397607

				380.87		2.397607

				380.89		2.397607

				380.91		2.397607

				380.93		2.397607

				380.95		2.397607

				380.98		2.397607

				381		2.397607

				381.02		2.397607

				381.04		2.397607

				381.06		2.397607

				381.08		2.397607

				381.1		2.402006

				381.12		2.402006

				381.15		2.402006

				381.17		2.402006

				381.19		2.402006

				381.21		2.402006

				381.23		2.402006

				381.25		2.402006

				381.27		2.402006

				381.29		2.402006

				381.32		2.402006

				381.34		2.402006

				381.36		2.402006

				381.38		2.402006

				381.4		2.402006

				381.42		2.402006

				381.44		2.402006

				381.46		2.402006

				381.49		2.402006

				381.51		2.397607

				381.53		2.402006

				381.55		2.402006

				381.57		2.402006

				381.59		2.402006

				381.61		2.402006

				381.63		2.402006

				381.65		2.402006

				381.68		2.402006

				381.7		2.402006

				381.72		2.402006

				381.74		2.402006

				381.76		2.402006

				381.78		2.402006

				381.8		2.402006

				381.82		2.402006

				381.85		2.402006

				381.87		2.402006

				381.89		2.402006

				381.91		2.402006

				381.93		2.402006

				381.95		2.402006

				381.97		2.402006

				381.99		2.402006

				382.02		2.402006

				382.04		2.402006

				382.06		2.402006

				382.08		2.402006

				382.1		2.402006

				382.12		2.402006

				382.14		2.402006

				382.16		2.402006

				382.19		2.402006

				382.21		2.402006

				382.23		2.402006

				382.25		2.402006

				382.27		2.402006

				382.29		2.402006

				382.31		2.402006

				382.33		2.402006

				382.36		2.402006

				382.38		2.402006

				382.4		2.402006

				382.42		2.402006

				382.44		2.402006

				382.46		2.402006

				382.48		2.402006

				382.5		2.406405

				382.53		2.406405

				382.55		2.406405

				382.57		2.406405

				382.59		2.406405

				382.61		2.406405

				382.63		2.406405

				382.65		2.406405

				382.67		2.406405

				382.7		2.406405

				382.72		2.406405

				382.74		2.406405

				382.76		2.406405

				382.78		2.406405

				382.8		2.406405

				382.82		2.406405

				382.84		2.406405

				382.86		2.406405

				382.89		2.406405

				382.91		2.406405

				382.93		2.406405

				382.95		2.406405

				382.97		2.406405

				382.99		2.406405

				383.01		2.406405

				383.03		2.406405

				383.06		2.406405

				383.08		2.406405

				383.1		2.406405

				383.12		2.406405

				383.14		2.406405

				383.16		2.406405

				383.18		2.406405

				383.2		2.406405

				383.23		2.406405

				383.25		2.406405

				383.27		2.406405

				383.29		2.406405

				383.31		2.406405

				383.33		2.406405

				383.35		2.406405

				383.37		2.406405

				383.39		2.406405

				383.42		2.406405

				383.44		2.406405

				383.46		2.406405

				383.48		2.406405

				383.5		2.406405

				383.52		2.406405

				383.54		2.406405

				383.56		2.406405

				383.59		2.406405

				383.61		2.410805

				383.63		2.410805

				383.65		2.410805

				383.67		2.410805

				383.69		2.410805

				383.71		2.410805

				383.73		2.410805

				383.76		2.410805

				383.78		2.410805

				383.8		2.410805

				383.82		2.410805

				383.84		2.410805

				383.86		2.410805

				383.88		2.410805

				383.9		2.410805

				383.93		2.410805

				383.95		2.410805

				383.97		2.410805

				383.99		2.410805

				384.01		2.410805

				384.03		2.410805

				384.05		2.410805

				384.07		2.410805

				384.09		2.410805

				384.12		2.406405

				384.14		2.406405

				384.16		2.406405

				384.18		2.406405

				384.2		2.406405

				384.22		2.406405

				384.24		2.406405

				384.26		2.406405

				384.29		2.406405

				384.31		2.406405

				384.33		2.406405

				384.35		2.410805

				384.37		2.410805

				384.39		2.406405

				384.41		2.406405

				384.43		2.406405

				384.46		2.406405

				384.48		2.406405

				384.5		2.406405

				384.52		2.406405

				384.54		2.406405

				384.56		2.406405

				384.58		2.406405

				384.6		2.406405

				384.62		2.406405

				384.65		2.406405

				384.67		2.406405

				384.69		2.406405

				384.71		2.406405

				384.73		2.406405

				384.75		2.406405

				384.77		2.406405

				384.79		2.406405

				384.82		2.406405

				384.84		2.406405

				384.86		2.406405

				384.88		2.406405

				384.9		2.406405

				384.92		2.406405

				384.94		2.406405

				384.96		2.406405

				384.99		2.406405

				385.01		2.406405

				385.03		2.406405

				385.05		2.406405

				385.07		2.406405

				385.09		2.406405

				385.11		2.406405

				385.13		2.406405

				385.15		2.406405

				385.18		2.406405

				385.2		2.406405

				385.22		2.406405

				385.24		2.406405

				385.26		2.406405

				385.28		2.406405

				385.3		2.406405

				385.32		2.406405

				385.35		2.406405

				385.37		2.406405

				385.39		2.406405

				385.41		2.406405

				385.43		2.406405

				385.45		2.406405

				385.47		2.406405

				385.49		2.406405

				385.52		2.406405

				385.54		2.406405

				385.56		2.406405

				385.58		2.406405

				385.6		2.406405

				385.62		2.406405

				385.64		2.406405

				385.66		2.406405

				385.68		2.406405

				385.71		2.406405

				385.73		2.406405

				385.75		2.406405

				385.77		2.406405

				385.79		2.406405

				385.81		2.406405

				385.83		2.406405

				385.85		2.406405

				385.88		2.406405

				385.9		2.406405

				385.92		2.406405

				385.94		2.406405

				385.96		2.406405

				385.98		2.406405

				386		2.406405

				386.02		2.406405

				386.05		2.406405

				386.07		2.406405

				386.09		2.402006

				386.11		2.406405

				386.13		2.406405

				386.15		2.406405

				386.17		2.406405

				386.19		2.406405

				386.22		2.406405

				386.24		2.406405

				386.26		2.406405

				386.28		2.406405

				386.3		2.406405

				386.32		2.406405

				386.34		2.406405

				386.36		2.406405

				386.38		2.406405

				386.41		2.406405

				386.43		2.406405

				386.45		2.402006

				386.47		2.402006

				386.49		2.402006

				386.51		2.402006

				386.53		2.402006

				386.55		2.402006

				386.58		2.402006

				386.6		2.402006

				386.62		2.402006

				386.64		2.402006

				386.66		2.402006

				386.68		2.402006

				386.7		2.402006

				386.72		2.402006

				386.75		2.402006

				386.77		2.402006

				386.79		2.402006

				386.81		2.402006

				386.83		2.402006

				386.85		2.402006

				386.87		2.402006

				386.89		2.402006

				386.92		2.402006

				386.94		2.402006

				386.96		2.402006

				386.98		2.402006

				387		2.402006

				387.02		2.402006

				387.04		2.402006

				387.06		2.402006

				387.08		2.402006

				387.11		2.402006

				387.13		2.402006

				387.15		2.402006

				387.17		2.402006

				387.19		2.402006

				387.21		2.402006

				387.23		2.402006

				387.25		2.402006

				387.28		2.402006

				387.3		2.402006

				387.32		2.402006

				387.34		2.402006

				387.36		2.402006

				387.38		2.402006

				387.4		2.402006

				387.42		2.402006

				387.45		2.402006

				387.47		2.402006

				387.49		2.402006

				387.51		2.402006

				387.53		2.402006

				387.55		2.402006

				387.57		2.402006

				387.59		2.406405

				387.61		2.406405

				387.64		2.406405

				387.66		2.402006

				387.68		2.402006

				387.7		2.406405

				387.72		2.402006

				387.74		2.406405

				387.76		2.406405

				387.78		2.406405

				387.81		2.406405

				387.83		2.406405

				387.85		2.406405

				387.87		2.406405

				387.89		2.406405

				387.91		2.406405

				387.93		2.406405

				387.95		2.406405

				387.97		2.406405

				388		2.406405

				388.02		2.406405

				388.04		2.406405

				388.06		2.406405

				388.08		2.406405

				388.1		2.406405

				388.12		2.406405

				388.14		2.406405

				388.17		2.406405

				388.19		2.406405

				388.21		2.406405

				388.23		2.406405

				388.25		2.406405

				388.27		2.406405

				388.29		2.406405

				388.31		2.406405

				388.34		2.406405

				388.36		2.406405

				388.38		2.406405

				388.4		2.406405

				388.42		2.406405

				388.44		2.410805

				388.46		2.410805

				388.48		2.410805

				388.5		2.406405

				388.53		2.410805

				388.55		2.410805

				388.57		2.410805

				388.59		2.410805

				388.61		2.410805

				388.63		2.410805

				388.65		2.410805

				388.67		2.410805

				388.7		2.410805

				388.72		2.410805

				388.74		2.410805

				388.76		2.410805

				388.78		2.410805

				388.8		2.410805

				388.82		2.410805

				388.84		2.415204

				388.86		2.415204

				388.89		2.415204

				388.91		2.410805

				388.93		2.410805

				388.95		2.415204

				388.97		2.415204

				388.99		2.415204

				389.01		2.415204

				389.03		2.415204

				389.06		2.415204

				389.08		2.415204

				389.1		2.415204

				389.12		2.415204

				389.14		2.415204

				389.16		2.415204

				389.18		2.415204

				389.2		2.415204

				389.22		2.415204

				389.25		2.415204

				389.27		2.415204

				389.29		2.419603

				389.31		2.419603

				389.33		2.419603

				389.35		2.419603

				389.37		2.419603

				389.39		2.419603

				389.42		2.419603

				389.44		2.419603

				389.46		2.419603

				389.48		2.419603

				389.5		2.419603

				389.52		2.419603

				389.54		2.419603

				389.56		2.419603

				389.58		2.419603

				389.61		2.419603

				389.63		2.419603

				389.65		2.419603

				389.67		2.419603

				389.69		2.419603

				389.71		2.419603

				389.73		2.419603

				389.75		2.419603

				389.78		2.419603

				389.8		2.419603

				389.82		2.419603

				389.84		2.419603

				389.86		2.419603

				389.88		2.419603

				389.9		2.419603

				389.92		2.419603

				389.94		2.419603

				389.97		2.419603

				389.99		2.419603

				390.01		2.419603

				390.03		2.419603

				390.05		2.419603

				390.07		2.419603

				390.09		2.424002

				390.11		2.424002

				390.14		2.424002

				390.16		2.424002

				390.18		2.424002

				390.2		2.424002

				390.22		2.424002

				390.24		2.424002

				390.26		2.424002

				390.28		2.424002

				390.3		2.424002

				390.33		2.424002

				390.35		2.424002

				390.37		2.424002

				390.39		2.424002

				390.41		2.424002

				390.43		2.424002

				390.45		2.424002

				390.47		2.424002

				390.5		2.424002

				390.52		2.424002

				390.54		2.424002

				390.56		2.424002

				390.58		2.424002

				390.6		2.424002

				390.62		2.424002

				390.64		2.424002

				390.66		2.424002

				390.69		2.424002

				390.71		2.424002

				390.73		2.424002

				390.75		2.424002

				390.77		2.424002

				390.79		2.424002

				390.81		2.424002

				390.83		2.424002

				390.86		2.424002

				390.88		2.424002

				390.9		2.424002

				390.92		2.424002

				390.94		2.424002

				390.96		2.424002

				390.98		2.424002

				391		2.424002

				391.02		2.424002

				391.05		2.424002

				391.07		2.424002

				391.09		2.424002

				391.11		2.424002

				391.13		2.424002

				391.15		2.424002

				391.17		2.424002

				391.19		2.424002

				391.21		2.424002

				391.24		2.424002

				391.26		2.424002

				391.28		2.424002

				391.3		2.424002

				391.32		2.424002

				391.34		2.424002

				391.36		2.424002

				391.38		2.424002

				391.41		2.424002

				391.43		2.424002

				391.45		2.424002

				391.47		2.424002

				391.49		2.424002

				391.51		2.424002

				391.53		2.424002

				391.55		2.424002

				391.57		2.424002

				391.6		2.424002

				391.62		2.424002

				391.64		2.424002

		Results:

		Onset		X1		188.46		°C

				Y1		93.142		%

				X2		253.76		°C

				Y2		15.16		%

				Onset X		216.87		°C

				Onset Y		84.392		%





image1.png

110

100

2

Weight % (%) —— ——

8

0

Fom e e i e

07282

Derivative Weight % (%imin)

2

2

3208

150

200
Temperature (C)

2059
65







image21.emf
RT54-1.0GNP-1.0M WCNT.xlsx


RT54-1.0GNP-1.0MWCNT.xlsx
Sheet1

		Method Filename:		C:\Program Files (x86)\PerkinElmer\Pyris\data\Anas\21052024\RT54-MWCNT 0.2 (GNP 1.0-MW 1.0).t6d

		Sample ID:		RT54-MWCNT 0.2 (GNP 1.0-MW 1.0)

		Step:		1

		Data		Sample Temperature (°C)		Weight % (%)

				30.06		99.99188

				30.06		99.99594

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99594

				30.06		99.99594

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.06		99.99188

				30.05		99.99188

				30.05		99.99188

				30.05		99.99188

				30.05		99.99188

				30.05		99.99188

				30.05		99.99188

				30.05		99.99188

				30.05		99.99188

				30.05		99.99188

				30.05		99.99188

				30.05		99.99188

				30.05		99.99188

				30.05		99.99188

				30.05		99.99188

				30.05		99.99188

				30.05		99.99188

				30.05		99.99188

				30.05		99.99188

				30.05		99.99188

				30.05		99.99188

				30.05		99.99188

				30.05		99.99188

				30.05		99.99188

				30.05		99.99188

				30.05		99.99188

				30.05		99.99188

				30.05		99.99188

				30.05		99.99188

				30.05		99.99594

				30.05		99.99594

				30.05		99.99594

				30.05		99.99594

				30.05		99.99594

				30.05		99.99594

				30.05		99.99594

				30.05		99.99594

				30.05		99.99594

				30.05		99.99594

				30.05		99.99594

				30.05		99.99594

				30.05		100

				30.05		100

				30.05		100

				30.05		100

				30.05		100

				30.05		100

				30.05		100

				30.05		100

				30.05		100

				30.05		100

				30.05		100

				30.05		100

				30.05		100

				30.05		100

				30.05		100.0041

				30.05		100.0041

				30.05		100.0041

				30.05		100.0041

				30.05		100.0041

				30.05		100.0041

				30.05		100.0041

				30.05		100.0041

				30.05		100.0041

				30.05		100.0041

				30.05		100.0041

				30.05		100.0041

				30.05		100.0041

				30.05		100.0041

				30.05		100.0041

				30.05		100.0041

				30.05		100.0081

				30.05		100.0081

				30.05		100.0081

				30.05		100.0081

				30.05		100.0081

				30.06		100.0081

				30.06		100.0081

				30.06		100.0081

				30.06		100.0122

				30.06		100.0122

				30.06		100.0122

				30.06		100.0122

				30.06		100.0122

				30.06		100.0122

				30.06		100.0122

				30.06		100.0162

				30.06		100.0162

				30.07		100.0162

				30.07		100.0162

				30.07		100.0162

				30.07		100.0203

				30.07		100.0203

				30.07		100.0203

				30.07		100.0244

				30.07		100.0244

				30.07		100.0244

				30.08		100.0244

				30.08		100.0244

				30.08		100.0244

				30.08		100.0284

				30.08		100.0284

				30.08		100.0284

				30.09		100.0284

				30.09		100.0325

				30.09		100.0325

				30.09		100.0325

				30.09		100.0325

				30.09		100.0366

				30.1		100.0366

				30.1		100.0366

				30.1		100.0366

				30.1		100.0366

				30.1		100.0366

				30.11		100.0366

				30.11		100.0406

				30.11		100.0406

				30.11		100.0406

				30.11		100.0406

				30.12		100.0447

				30.12		100.0447

				30.12		100.0406

				30.12		100.0447

				30.13		100.0447

				30.13		100.0447

				30.13		100.0447

				30.13		100.0447

				30.14		100.0447

				30.14		100.0447

				30.14		100.0447

				30.15		100.0487

				30.15		100.0487

				30.15		100.0487

				30.15		100.0487

				30.16		100.0487

				30.16		100.0487

				30.16		100.0528

				30.17		100.0528

				30.17		100.0528

				30.17		100.0528

				30.18		100.0528

				30.18		100.0569

				30.18		100.0569

				30.19		100.0569

				30.19		100.0569

				30.19		100.0569

				30.2		100.0569

				30.2		100.0609

				30.2		100.0609

				30.21		100.0609

				30.21		100.0609

				30.21		100.065

				30.22		100.065

				30.22		100.065

				30.23		100.065

				30.23		100.065

				30.23		100.065

				30.24		100.065

				30.24		100.065

				30.25		100.0691

				30.25		100.0691

				30.25		100.0691

				30.26		100.0691

				30.26		100.0691

				30.27		100.0731

				30.27		100.0731

				30.27		100.0731

				30.28		100.0731

				30.28		100.0731

				30.29		100.0731

				30.29		100.0731

				30.3		100.0731

				30.3		100.0731

				30.31		100.0731

				30.31		100.0772

				30.32		100.0772

				30.32		100.0772

				30.32		100.0772

				30.33		100.0772

				30.33		100.0772

				30.34		100.0772

				30.34		100.0772

				30.35		100.0772

				30.35		100.0812

				30.36		100.0772

				30.36		100.0812

				30.37		100.0812

				30.37		100.0812

				30.38		100.0812

				30.38		100.0812

				30.39		100.0853

				30.4		100.0853

				30.4		100.0853

				30.41		100.0853

				30.41		100.0853

				30.42		100.0853

				30.42		100.0853

				30.43		100.0853

				30.43		100.0853

				30.44		100.0853

				30.44		100.0853

				30.45		100.0853

				30.46		100.0853

				30.46		100.0853

				30.47		100.0853

				30.47		100.0894

				30.48		100.0894

				30.48		100.0894

				30.49		100.0894

				30.5		100.0894

				30.5		100.0894

				30.51		100.0894

				30.51		100.0934

				30.52		100.0934

				30.53		100.0934

				30.53		100.0934

				30.54		100.0934

				30.54		100.0934

				30.55		100.0934

				30.56		100.0934

				30.56		100.0934

				30.57		100.0934

				30.58		100.0934

				30.58		100.0934

				30.59		100.0975

				30.6		100.0975

				30.6		100.0975

				30.61		100.0975

				30.61		100.0975

				30.62		100.0975

				30.63		100.0975

				30.63		100.0975

				30.64		100.0975

				30.65		100.1016

				30.65		100.1016

				30.66		100.1016

				30.67		100.1016

				30.67		100.1016

				30.68		100.1016

				30.69		100.1016

				30.7		100.1016

				30.7		100.1016

				30.71		100.1016

				30.72		100.1016

				30.72		100.1016

				30.73		100.1016

				30.74		100.1016

				30.74		100.1016

				30.75		100.1016

				30.76		100.1016

				30.77		100.1016

				30.77		100.1056

				30.78		100.1056

				30.79		100.1056

				30.79		100.1056

				30.8		100.1056

				30.81		100.1056

				30.82		100.1056

				30.82		100.1056

				30.83		100.1056

				30.84		100.1056

				30.85		100.1056

				30.85		100.1056

				30.86		100.1056

				30.87		100.1097

				30.88		100.1056

				30.88		100.1097

				30.89		100.1097

				30.9		100.1056

				30.91		100.1097

				30.91		100.1097

				30.92		100.1097

				30.93		100.1097

				30.94		100.1097

				30.95		100.1097

				30.95		100.1097

				30.96		100.1137

				30.97		100.1137

				30.98		100.1137

				30.99		100.1137

				30.99		100.1137

				31		100.1137

				31.01		100.1137

				31.02		100.1137

				31.03		100.1137

				31.03		100.1137

				31.04		100.1137

				31.05		100.1137

				31.06		100.1137

				31.07		100.1137

				31.07		100.1137

				31.08		100.1137

				31.09		100.1137

				31.1		100.1137

				31.11		100.1137

				31.12		100.1178

				31.12		100.1178

				31.13		100.1178

				31.14		100.1178

				31.15		100.1178

				31.16		100.1178

				31.17		100.1178

				31.17		100.1178

				31.18		100.1178

				31.19		100.1178

				31.2		100.1178

				31.21		100.1178

				31.22		100.1178

				31.23		100.1178

				31.24		100.1178

				31.24		100.1178

				31.25		100.1178

				31.26		100.1178

				31.27		100.1178

				31.28		100.1178

				31.29		100.1178

				31.3		100.1178

				31.31		100.1178

				31.31		100.1178

				31.32		100.1178

				31.33		100.1219

				31.34		100.1219

				31.35		100.1219

				31.36		100.1219

				31.37		100.1219

				31.38		100.1219

				31.39		100.1219

				31.4		100.1219

				31.4		100.1219

				31.41		100.1219

				31.42		100.1219

				31.43		100.1219

				31.44		100.1219

				31.45		100.1219

				31.46		100.1219

				31.47		100.1219

				31.48		100.1219

				31.49		100.1219

				31.5		100.1219

				31.51		100.1219

				31.52		100.1219

				31.52		100.1219

				31.53		100.1219

				31.54		100.1219

				31.55		100.1259

				31.56		100.1219

				31.57		100.1219

				31.58		100.1259

				31.59		100.1259

				31.6		100.1259

				31.61		100.1259

				31.62		100.1259

				31.63		100.1259

				31.64		100.1259

				31.65		100.1259

				31.66		100.1259

				31.67		100.1259

				31.68		100.1259

				31.69		100.1259

				31.7		100.1259

				31.71		100.1259

				31.72		100.1259

				31.73		100.1259

				31.74		100.1259

				31.75		100.13

				31.76		100.13

				31.77		100.13

				31.78		100.13

				31.79		100.13

				31.8		100.13

				31.81		100.13

				31.82		100.13

				31.83		100.13

				31.84		100.13

				31.85		100.13

				31.86		100.13

				31.87		100.13

				31.88		100.13

				31.89		100.134

				31.9		100.134

				31.91		100.134

				31.92		100.134

				31.93		100.134

				31.94		100.134

				31.95		100.134

				31.96		100.134

				31.97		100.134

				31.98		100.134

				31.99		100.1381

				32		100.1381

				32.01		100.1381

				32.02		100.1381

				32.03		100.1381

				32.04		100.1381

				32.05		100.1381

				32.06		100.1381

				32.07		100.1381

				32.08		100.1381

				32.09		100.1381

				32.1		100.1381

				32.12		100.1381

				32.13		100.1381

				32.14		100.1381

				32.15		100.1381

				32.16		100.1422

				32.17		100.1381

				32.18		100.1422

				32.19		100.1422

				32.2		100.1422

				32.21		100.1422

				32.22		100.1422

				32.23		100.1422

				32.24		100.1422

				32.26		100.1422

				32.27		100.1422

				32.28		100.1422

				32.29		100.1422

				32.3		100.1422

				32.31		100.1422

				32.32		100.1422

				32.33		100.1462

				32.34		100.1462

				32.35		100.1462

				32.37		100.1462

				32.38		100.1462

				32.39		100.1462

				32.4		100.1462

				32.41		100.1462

				32.42		100.1462

				32.43		100.1462

				32.44		100.1462

				32.45		100.1462

				32.47		100.1462

				32.48		100.1462

				32.49		100.1503

				32.5		100.1503

				32.51		100.1503

				32.52		100.1503

				32.53		100.1503

				32.55		100.1503

				32.56		100.1503

				32.57		100.1503

				32.58		100.1503

				32.59		100.1503

				32.6		100.1503

				32.61		100.1503

				32.63		100.1503

				32.64		100.1503

				32.65		100.1503

				32.66		100.1503

				32.67		100.1503

				32.68		100.1503

				32.7		100.1503

				32.71		100.1503

				32.72		100.1503

				32.73		100.1544

				32.74		100.1544

				32.75		100.1544

				32.77		100.1544

				32.78		100.1544

				32.79		100.1544

				32.8		100.1544

				32.81		100.1544

				32.82		100.1544

				32.84		100.1544

				32.85		100.1544

				32.86		100.1544

				32.87		100.1544

				32.88		100.1544

				32.9		100.1584

				32.91		100.1584

				32.92		100.1584

				32.93		100.1584

				32.94		100.1584

				32.96		100.1584

				32.97		100.1584

				32.98		100.1584

				32.99		100.1584

				33		100.1584

				33.02		100.1584

				33.03		100.1584

				33.04		100.1584

				33.05		100.1584

				33.06		100.1584

				33.08		100.1584

				33.09		100.1584

				33.1		100.1584

				33.11		100.1584

				33.13		100.1584

				33.14		100.1584

				33.15		100.1584

				33.16		100.1584

				33.18		100.1625

				33.19		100.1625

				33.2		100.1625

				33.21		100.1625

				33.23		100.1625

				33.24		100.1625

				33.25		100.1625

				33.26		100.1625

				33.27		100.1625

				33.29		100.1625

				33.3		100.1625

				33.31		100.1625

				33.32		100.1625

				33.34		100.1625

				33.35		100.1625

				33.36		100.1625

				33.38		100.1665

				33.39		100.1665

				33.4		100.1665

				33.41		100.1665

				33.43		100.1665

				33.44		100.1665

				33.45		100.1665

				33.46		100.1665

				33.48		100.1665

				33.49		100.1665

				33.5		100.1665

				33.52		100.1665

				33.53		100.1665

				33.54		100.1665

				33.55		100.1665

				33.57		100.1706

				33.58		100.1706

				33.59		100.1706

				33.61		100.1706

				33.62		100.1706

				33.63		100.1706

				33.64		100.1706

				33.66		100.1706

				33.67		100.1706

				33.68		100.1706

				33.7		100.1706

				33.71		100.1706

				33.72		100.1706

				33.74		100.1706

				33.75		100.1747

				33.76		100.1747

				33.77		100.1747

				33.79		100.1747

				33.8		100.1747

				33.81		100.1747

				33.83		100.1747

				33.84		100.1747

				33.85		100.1747

				33.87		100.1747

				33.88		100.1747

				33.89		100.1747

				33.91		100.1787

				33.92		100.1787

				33.93		100.1787

				33.95		100.1787

				33.96		100.1787

				33.97		100.1787

				33.99		100.1787

				34		100.1787

				34.01		100.1787

				34.03		100.1787

				34.04		100.1787

				34.05		100.1787

				34.07		100.1787

				34.08		100.1787

				34.09		100.1787

				34.11		100.1787

				34.12		100.1787

				34.13		100.1787

				34.15		100.1787

				34.16		100.1787

				34.18		100.1828

				34.19		100.1828

				34.2		100.1828

				34.22		100.1828

				34.23		100.1828

				34.24		100.1828

				34.26		100.1828

				34.27		100.1828

				34.28		100.1828

				34.3		100.1828

				34.31		100.1828

				34.33		100.1828

				34.34		100.1828

				34.35		100.1828

				34.37		100.1828

				34.38		100.1828

				34.39		100.1828

				34.41		100.1828

				34.42		100.1869

				34.44		100.1828

				34.45		100.1869

				34.46		100.1869

				34.48		100.1869

				34.49		100.1869

				34.51		100.1869

				34.52		100.1869

				34.53		100.1869

				34.55		100.1869

				34.56		100.1869

				34.58		100.1869

				34.59		100.1869

				34.6		100.1869

				34.62		100.1869

				34.63		100.1869

				34.65		100.1869

				34.66		100.1869

				34.67		100.1869

				34.69		100.1869

				34.7		100.1869

				34.72		100.1869

				34.73		100.1909

				34.74		100.1909

				34.76		100.1909

				34.77		100.1909

				34.79		100.1909

				34.8		100.1909

				34.82		100.1909

				34.83		100.1909

				34.84		100.1909

				34.86		100.1909

				34.87		100.1909

				34.89		100.1909

				34.9		100.1909

				34.92		100.1909

				34.93		100.1909

				34.94		100.1909

				34.96		100.1909

				34.97		100.1909

				34.99		100.1909

				35		100.1909

				35.02		100.195

				35.03		100.195

				35.04		100.195

				35.06		100.195

				35.07		100.195

				35.09		100.195

				35.1		100.195

				35.12		100.195

				35.13		100.195

				35.15		100.195

				35.16		100.195

				35.17		100.195

				35.19		100.195

				35.2		100.195

				35.22		100.199

				35.23		100.199

				35.25		100.199

				35.26		100.199

				35.28		100.199

				35.29		100.199

				35.31		100.199

				35.32		100.199

				35.34		100.199

				35.35		100.199

				35.36		100.199

				35.38		100.199

				35.39		100.199

				35.41		100.199

				35.42		100.199

				35.44		100.199

				35.45		100.199

				35.47		100.2031

				35.48		100.2031

				35.5		100.2031

				35.51		100.2031

				35.53		100.2031

				35.54		100.2031

				35.56		100.2031

				35.57		100.2031

				35.59		100.2031

				35.6		100.2031

				35.62		100.2031

				35.63		100.2031

				35.65		100.2031

				35.66		100.2031

				35.68		100.2072

				35.69		100.2072

				35.71		100.2072

				35.72		100.2072

				35.74		100.2072

				35.75		100.2072

				35.77		100.2072

				35.78		100.2072

				35.8		100.2072

				35.81		100.2072

				35.83		100.2072

				35.84		100.2072

				35.86		100.2072

				35.87		100.2072

				35.89		100.2072

				35.9		100.2112

				35.92		100.2112

				35.93		100.2112

				35.95		100.2112

				35.96		100.2112

				35.98		100.2112

				35.99		100.2112

				36.01		100.2112

				36.02		100.2112

				36.04		100.2112

				36.05		100.2112

				36.07		100.2153

				36.09		100.2153

				36.1		100.2153

				36.12		100.2153

				36.13		100.2153

				36.15		100.2153

				36.16		100.2153

				36.18		100.2153

				36.19		100.2153

				36.21		100.2153

				36.22		100.2153

				36.24		100.2153

				36.25		100.2153

				36.27		100.2153

				36.28		100.2194

				36.3		100.2194

				36.32		100.2194

				36.33		100.2194

				36.35		100.2194

				36.36		100.2194

				36.38		100.2194

				36.39		100.2194

				36.41		100.2194

				36.42		100.2194

				36.44		100.2234

				36.46		100.2234

				36.47		100.2234

				36.49		100.2234

				36.5		100.2234

				36.52		100.2234

				36.53		100.2234

				36.55		100.2234

				36.56		100.2234

				36.58		100.2234

				36.6		100.2234

				36.61		100.2234

				36.63		100.2234

				36.64		100.2234

				36.66		100.2234

				36.67		100.2234

				36.69		100.2275

				36.71		100.2275

				36.72		100.2275

				36.74		100.2275

				36.75		100.2275

				36.77		100.2275

				36.78		100.2275

				36.8		100.2275

				36.82		100.2275

				36.83		100.2275

				36.85		100.2275

				36.86		100.2275

				36.88		100.2315

				36.89		100.2315

				36.91		100.2315

				36.93		100.2315

				36.94		100.2315

				36.96		100.2315

				36.97		100.2315

				36.99		100.2315

				37.01		100.2315

				37.02		100.2315

				37.04		100.2356

				37.05		100.2356

				37.07		100.2356

				37.09		100.2356

				37.1		100.2356

				37.12		100.2356

				37.13		100.2356

				37.15		100.2356

				37.17		100.2356

				37.18		100.2356

				37.2		100.2356

				37.21		100.2356

				37.23		100.2356

				37.25		100.2356

				37.26		100.2356

				37.28		100.2356

				37.29		100.2356

				37.31		100.2356

				37.33		100.2397

				37.34		100.2397

				37.36		100.2397

				37.37		100.2397

				37.39		100.2397

				37.41		100.2397

				37.42		100.2397

				37.44		100.2397

				37.46		100.2397

				37.47		100.2397

				37.49		100.2397

				37.5		100.2397

				37.52		100.2397

				37.54		100.2397

				37.55		100.2437

				37.57		100.2437

				37.59		100.2437

				37.6		100.2437

				37.62		100.2437

				37.63		100.2437

				37.65		100.2437

				37.67		100.2437

				37.68		100.2437

				37.7		100.2437

				37.72		100.2478

				37.73		100.2478

				37.75		100.2478

				37.76		100.2478

				37.78		100.2478

				37.8		100.2478

				37.81		100.2478

				37.83		100.2478

				37.85		100.2478

				37.86		100.2478

				37.88		100.2478

				37.9		100.2478

				37.91		100.2478

				37.93		100.2478

				37.95		100.2478

				37.96		100.2478

				37.98		100.2478

				37.99		100.2478

				38.01		100.2518

				38.03		100.2518

				38.04		100.2518

				38.06		100.2518

				38.08		100.2518

				38.09		100.2518

				38.11		100.2518

				38.13		100.2518

				38.14		100.2518

				38.16		100.2518

				38.18		100.2518

				38.19		100.2518

				38.21		100.2518

				38.23		100.2518

				38.24		100.2518

				38.26		100.2518

				38.28		100.2518

				38.29		100.2518

				38.31		100.2559

				38.33		100.2559

				38.34		100.2559

				38.36		100.2559

				38.38		100.2559

				38.39		100.2559

				38.41		100.2559

				38.43		100.2559

				38.44		100.2559

				38.46		100.2559

				38.48		100.2559

				38.49		100.2559

				38.51		100.2559

				38.53		100.2559

				38.54		100.2559

				38.56		100.2559

				38.58		100.2559

				38.59		100.2559

				38.61		100.2559

				38.63		100.2559

				38.65		100.2559

				38.66		100.2559

				38.68		100.2559

				38.7		100.2559

				38.71		100.2559

				38.73		100.2559

				38.75		100.2559

				38.76		100.2559

				38.78		100.2559

				38.8		100.2559

				38.81		100.2559

				38.83		100.2559

				38.85		100.2559

				38.86		100.2559

				38.88		100.2559

				38.9		100.2559

				38.92		100.2559

				38.93		100.26

				38.95		100.26

				38.97		100.26

				38.98		100.26

				39		100.26

				39.02		100.26

				39.03		100.26

				39.05		100.26

				39.07		100.26

				39.09		100.26

				39.1		100.26

				39.12		100.26

				39.14		100.26

				39.15		100.26

				39.17		100.26

				39.19		100.26

				39.21		100.26

				39.22		100.26

				39.24		100.26

				39.26		100.26

				39.27		100.26

				39.29		100.26

				39.31		100.26

				39.33		100.26

				39.34		100.26

				39.36		100.26

				39.38		100.26

				39.39		100.26

				39.41		100.26

				39.43		100.26

				39.45		100.26

				39.46		100.26

				39.48		100.26

				39.5		100.26

				39.52		100.26

				39.53		100.264

				39.55		100.264

				39.57		100.264

				39.58		100.264

				39.6		100.264

				39.62		100.264

				39.64		100.264

				39.65		100.264

				39.67		100.264

				39.69		100.264

				39.71		100.264

				39.72		100.264

				39.74		100.264

				39.76		100.264

				39.77		100.264

				39.79		100.264

				39.81		100.264

				39.83		100.264

				39.84		100.264

				39.86		100.264

				39.88		100.2681

				39.9		100.2681

				39.91		100.264

				39.93		100.2681

				39.95		100.264

				39.97		100.2681

				39.98		100.264

				40		100.264

				40.02		100.2681

				40.04		100.2681

				40.05		100.2681

				40.07		100.2681

				40.09		100.2681

				40.11		100.264

				40.12		100.2681

				40.14		100.2681

				40.16		100.2681

				40.18		100.2681

				40.19		100.2681

				40.21		100.2681

				40.23		100.2681

				40.25		100.2681

				40.26		100.2681

				40.28		100.2681

				40.3		100.2722

				40.32		100.2722

				40.33		100.2722

				40.35		100.2722

				40.37		100.2722

				40.39		100.2722

				40.4		100.2722

				40.42		100.2722

				40.44		100.2722

				40.46		100.2722

				40.48		100.2722

				40.49		100.2722

				40.51		100.2722

				40.53		100.2722

				40.55		100.2722

				40.56		100.2722

				40.58		100.2722

				40.6		100.2762

				40.62		100.2762

				40.63		100.2762

				40.65		100.2762

				40.67		100.2762

				40.69		100.2762

				40.71		100.2762

				40.72		100.2762

				40.74		100.2762

				40.76		100.2762

				40.78		100.2762

				40.79		100.2762

				40.81		100.2762

				40.83		100.2762

				40.85		100.2762

				40.87		100.2762

				40.88		100.2762

				40.9		100.2762

				40.92		100.2762

				40.94		100.2803

				40.95		100.2803

				40.97		100.2803

				40.99		100.2803

				41.01		100.2803

				41.03		100.2803

				41.04		100.2803

				41.06		100.2803

				41.08		100.2803

				41.1		100.2803

				41.12		100.2803

				41.13		100.2803

				41.15		100.2803

				41.17		100.2803

				41.19		100.2803

				41.21		100.2803

				41.22		100.2803

				41.24		100.2803

				41.26		100.2803

				41.28		100.2803

				41.29		100.2803

				41.31		100.2843

				41.33		100.2843

				41.35		100.2843

				41.37		100.2843

				41.38		100.2843

				41.4		100.2843

				41.42		100.2843

				41.44		100.2843

				41.46		100.2843

				41.47		100.2843

				41.49		100.2843

				41.51		100.2843

				41.53		100.2843

				41.55		100.2843

				41.56		100.2843

				41.58		100.2843

				41.6		100.2843

				41.62		100.2843

				41.64		100.2843

				41.66		100.2843

				41.67		100.2843

				41.69		100.2843

				41.71		100.2843

				41.73		100.2843

				41.75		100.2884

				41.76		100.2884

				41.78		100.2884

				41.8		100.2884

				41.82		100.2884

				41.84		100.2884

				41.85		100.2884

				41.87		100.2884

				41.89		100.2884

				41.91		100.2884

				41.93		100.2884

				41.95		100.2884

				41.96		100.2884

				41.98		100.2884

				42		100.2884

				42.02		100.2884

				42.04		100.2884

				42.05		100.2884

				42.07		100.2884

				42.09		100.2884

				42.11		100.2925

				42.13		100.2925

				42.15		100.2925

				42.16		100.2925

				42.18		100.2925

				42.2		100.2925

				42.22		100.2925

				42.24		100.2925

				42.26		100.2925

				42.27		100.2925

				42.29		100.2925

				42.31		100.2925

				42.33		100.2925

				42.35		100.2925

				42.37		100.2925

				42.38		100.2925

				42.4		100.2925

				42.42		100.2925

				42.44		100.2925

				42.46		100.2925

				42.48		100.2925

				42.49		100.2925

				42.51		100.2925

				42.53		100.2925

				42.55		100.2925

				42.57		100.2925

				42.59		100.2925

				42.6		100.2925

				42.62		100.2925

				42.64		100.2925

				42.66		100.2925

				42.68		100.2925

				42.7		100.2925

				42.71		100.2925

				42.73		100.2925

				42.75		100.2925

				42.77		100.2925

				42.79		100.2925

				42.81		100.2925

				42.82		100.2925

				42.84		100.2925

				42.86		100.2925

				42.88		100.2925

				42.9		100.2965

				42.92		100.2965

				42.94		100.2925

				42.95		100.2965

				42.97		100.2965

				42.99		100.2965

				43.01		100.2965

				43.03		100.2965

				43.05		100.2965

				43.06		100.2965

				43.08		100.2965

				43.1		100.2965

				43.12		100.2965

				43.14		100.2965

				43.16		100.2965

				43.18		100.2965

				43.19		100.2965

				43.21		100.2965

				43.23		100.2965

				43.25		100.2965

				43.27		100.2965

				43.29		100.2965

				43.31		100.2965

				43.32		100.3006

				43.34		100.3006

				43.36		100.3006

				43.38		100.3006

				43.4		100.3006

				43.42		100.3006

				43.44		100.3006

				43.45		100.3006

				43.47		100.3006

				43.49		100.3006

				43.51		100.3006

				43.53		100.3006

				43.55		100.3006

				43.57		100.3006

				43.59		100.3006

				43.6		100.3006

				43.62		100.3006

				43.64		100.3006

				43.66		100.3006

				43.68		100.3006

				43.7		100.3006

				43.72		100.3047

				43.73		100.3047

				43.75		100.3047

				43.77		100.3047

				43.79		100.3047

				43.81		100.3047

				43.83		100.3047

				43.85		100.3047

				43.87		100.3047

				43.88		100.3047

				43.9		100.3047

				43.92		100.3047

				43.94		100.3047

				43.96		100.3047

				43.98		100.3047

				44		100.3047

				44.02		100.3047

				44.03		100.3047

				44.05		100.3047

				44.07		100.3087

				44.09		100.3047

				44.11		100.3087

				44.13		100.3087

				44.15		100.3087

				44.17		100.3087

				44.18		100.3087

				44.2		100.3087

				44.22		100.3087

				44.24		100.3087

				44.26		100.3087

				44.28		100.3087

				44.3		100.3087

				44.32		100.3087

				44.34		100.3087

				44.35		100.3087

				44.37		100.3087

				44.39		100.3087

				44.41		100.3087

				44.43		100.3087

				44.45		100.3128

				44.47		100.3128

				44.49		100.3128

				44.5		100.3128

				44.52		100.3128

				44.54		100.3128

				44.56		100.3128

				44.58		100.3128

				44.6		100.3128

				44.62		100.3128

				44.64		100.3128

				44.66		100.3128

				44.68		100.3128

				44.69		100.3128

				44.71		100.3128

				44.73		100.3128

				44.75		100.3128

				44.77		100.3128

				44.79		100.3128

				44.81		100.3128

				44.83		100.3128

				44.85		100.3128

				44.86		100.3128

				44.88		100.3128

				44.9		100.3128

				44.92		100.3128

				44.94		100.3128

				44.96		100.3128

				44.98		100.3128

				45		100.3128

				45.02		100.3128

				45.04		100.3128

				45.05		100.3128

				45.07		100.3128

				45.09		100.3128

				45.11		100.3128

				45.13		100.3128

				45.15		100.3128

				45.17		100.3128

				45.19		100.3128

				45.21		100.3128

				45.23		100.3128

				45.24		100.3128

				45.26		100.3128

				45.28		100.3128

				45.3		100.3128

				45.32		100.3128

				45.34		100.3128

				45.36		100.3128

				45.38		100.3128

				45.4		100.3128

				45.42		100.3168

				45.44		100.3168

				45.45		100.3128

				45.47		100.3128

				45.49		100.3128

				45.51		100.3128

				45.53		100.3128

				45.55		100.3128

				45.57		100.3128

				45.59		100.3128

				45.61		100.3128

				45.63		100.3128

				45.65		100.3128

				45.66		100.3128

				45.68		100.3128

				45.7		100.3128

				45.72		100.3128

				45.74		100.3128

				45.76		100.3128

				45.78		100.3128

				45.8		100.3128

				45.82		100.3128

				45.84		100.3128

				45.86		100.3128

				45.88		100.3128

				45.89		100.3128

				45.91		100.3128

				45.93		100.3128

				45.95		100.3128

				45.97		100.3128

				45.99		100.3128

				46.01		100.3128

				46.03		100.3128

				46.05		100.3128

				46.07		100.3128

				46.09		100.3128

				46.11		100.3128

				46.13		100.3128

				46.14		100.3128

				46.16		100.3128

				46.18		100.3128

				46.2		100.3128

				46.22		100.3087

				46.24		100.3087

				46.26		100.3128

				46.28		100.3128

				46.3		100.3128

				46.32		100.3087

				46.34		100.3087

				46.36		100.3087

				46.38		100.3087

				46.4		100.3128

				46.41		100.3128

				46.43		100.3128

				46.45		100.3128

				46.47		100.3128

				46.49		100.3128

				46.51		100.3128

				46.53		100.3128

				46.55		100.3128

				46.57		100.3128

				46.59		100.3128

				46.61		100.3128

				46.63		100.3128

				46.65		100.3128

				46.67		100.3128

				46.68		100.3128

				46.7		100.3128

				46.72		100.3128

				46.74		100.3128

				46.76		100.3128

				46.78		100.3128

				46.8		100.3128

				46.82		100.3128

				46.84		100.3128

				46.86		100.3128

				46.88		100.3128

				46.9		100.3128

				46.92		100.3128

				46.94		100.3128

				46.96		100.3128

				46.98		100.3128

				46.99		100.3128

				47.01		100.3128

				47.03		100.3128

				47.05		100.3128

				47.07		100.3128

				47.09		100.3128

				47.11		100.3128

				47.13		100.3128

				47.15		100.3128

				47.17		100.3128

				47.19		100.3168

				47.21		100.3168

				47.23		100.3168

				47.25		100.3168

				47.27		100.3168

				47.29		100.3168

				47.31		100.3168

				47.32		100.3168

				47.34		100.3168

				47.36		100.3168

				47.38		100.3168

				47.4		100.3168

				47.42		100.3168

				47.44		100.3168

				47.46		100.3168

				47.48		100.3168

				47.5		100.3168

				47.52		100.3209

				47.54		100.3168

				47.56		100.3168

				47.58		100.3209

				47.6		100.3209

				47.62		100.3209

				47.64		100.3209

				47.66		100.3209

				47.68		100.3209

				47.7		100.3209

				47.71		100.3209

				47.73		100.3209

				47.75		100.3209

				47.77		100.3209

				47.79		100.3209

				47.81		100.3209

				47.83		100.3209

				47.85		100.325

				47.87		100.3209

				47.89		100.325

				47.91		100.325

				47.93		100.325

				47.95		100.325

				47.97		100.325

				47.99		100.325

				48.01		100.325

				48.03		100.325

				48.05		100.325

				48.07		100.325

				48.09		100.325

				48.11		100.325

				48.13		100.325

				48.14		100.325

				48.16		100.329

				48.18		100.325

				48.2		100.329

				48.22		100.329

				48.24		100.329

				48.26		100.329

				48.28		100.329

				48.3		100.329

				48.32		100.329

				48.34		100.329

				48.36		100.329

				48.38		100.329

				48.4		100.329

				48.42		100.329

				48.44		100.329

				48.46		100.329

				48.48		100.329

				48.5		100.329

				48.52		100.3331

				48.54		100.3331

				48.56		100.3331

				48.58		100.3331

				48.6		100.329

				48.62		100.3331

				48.64		100.3331

				48.66		100.3331

				48.67		100.3331

				48.69		100.3331

				48.71		100.3331

				48.73		100.3331

				48.75		100.3331

				48.77		100.3331

				48.79		100.3331

				48.81		100.3331

				48.83		100.3331

				48.85		100.3331

				48.87		100.3331

				48.89		100.3331

				48.91		100.3331

				48.93		100.3331

				48.95		100.3331

				48.97		100.3331

				48.99		100.3331

				49.01		100.3331

				49.03		100.3331

				49.05		100.3331

				49.07		100.3331

				49.09		100.3331

				49.11		100.3372

				49.13		100.3331

				49.15		100.3331

				49.17		100.3331

				49.19		100.3372

				49.21		100.3331

				49.23		100.3372

				49.25		100.3372

				49.27		100.3372

				49.29		100.3372

				49.31		100.3372

				49.33		100.3372

				49.35		100.3372

				49.37		100.3372

				49.39		100.3372

				49.41		100.3372

				49.42		100.3372

				49.44		100.3372

				49.46		100.3372

				49.48		100.3372

				49.5		100.3372

				49.52		100.3372

				49.54		100.3372

				49.56		100.3372

				49.58		100.3372

				49.6		100.3372

				49.62		100.3372

				49.64		100.3372

				49.66		100.3372

				49.68		100.3372

				49.7		100.3372

				49.72		100.3372

				49.74		100.3372

				49.76		100.3372

				49.78		100.3372

				49.8		100.3372

				49.82		100.3412

				49.84		100.3412

				49.86		100.3412

				49.88		100.3412

				49.9		100.3412

				49.92		100.3412

				49.94		100.3412

				49.96		100.3412

				49.98		100.3412

				50		100.3412

				50.02		100.3412

				50.04		100.3412

				50.06		100.3412

				50.08		100.3412

				50.1		100.3412

				50.12		100.3412

				50.14		100.3412

				50.16		100.3412

				50.18		100.3412

				50.2		100.3412

				50.22		100.3412

				50.24		100.3412

				50.26		100.3412

				50.28		100.3412

				50.3		100.3412

				50.32		100.3412

				50.34		100.3412

				50.36		100.3412

				50.38		100.3412

				50.4		100.3412

				50.42		100.3412

				50.44		100.3412

				50.46		100.3412

				50.48		100.3412

				50.5		100.3412

				50.52		100.3412

				50.54		100.3412

				50.56		100.3412

				50.58		100.3412

				50.6		100.3412

				50.62		100.3412

				50.64		100.3412

				50.66		100.3412

				50.68		100.3412

				50.7		100.3453

				50.72		100.3453

				50.74		100.3412

				50.76		100.3412

				50.78		100.3453

				50.8		100.3412

				50.82		100.3412

				50.84		100.3412

				50.86		100.3412

				50.88		100.3412

				50.9		100.3412

				50.92		100.3412

				50.94		100.3412

				50.96		100.3412

				50.98		100.3412

				51		100.3412

				51.02		100.3412

				51.04		100.3412

				51.06		100.3412

				51.08		100.3412

				51.1		100.3412

				51.12		100.3412

				51.14		100.3412

				51.16		100.3412

				51.18		100.3412

				51.2		100.3412

				51.22		100.3412

				51.24		100.3412

				51.26		100.3412

				51.28		100.3412

				51.3		100.3412

				51.32		100.3412

				51.34		100.3412

				51.36		100.3412

				51.38		100.3412

				51.4		100.3412

				51.42		100.3412

				51.44		100.3412

				51.46		100.3412

				51.48		100.3412

				51.5		100.3412

				51.52		100.3412

				51.54		100.3412

				51.56		100.3412

				51.58		100.3412

				51.6		100.3412

				51.62		100.3412

				51.64		100.3412

				51.66		100.3412

				51.68		100.3412

				51.7		100.3412

				51.72		100.3412

				51.74		100.3412

				51.76		100.3412

				51.78		100.3412

				51.8		100.3412

				51.82		100.3412

				51.84		100.3412

				51.86		100.3412

				51.88		100.3412

				51.9		100.3412

				51.92		100.3412

				51.94		100.3412

				51.96		100.3412

				51.98		100.3412

				52		100.3412

				52.02		100.3412

				52.04		100.3453

				52.06		100.3453

				52.08		100.3453

				52.1		100.3453

				52.12		100.3453

				52.14		100.3453

				52.16		100.3453

				52.18		100.3453

				52.2		100.3453

				52.22		100.3453

				52.24		100.3453

				52.26		100.3453

				52.28		100.3453

				52.3		100.3453

				52.32		100.3453

				52.34		100.3453

				52.36		100.3453

				52.38		100.3453

				52.4		100.3453

				52.42		100.3493

				52.44		100.3493

				52.46		100.3493

				52.48		100.3493

				52.5		100.3493

				52.52		100.3493

				52.54		100.3493

				52.56		100.3493

				52.58		100.3493

				52.6		100.3493

				52.62		100.3534

				52.64		100.3534

				52.66		100.3534

				52.68		100.3534

				52.7		100.3534

				52.72		100.3534

				52.74		100.3534

				52.76		100.3534

				52.78		100.3534

				52.8		100.3534

				52.82		100.3534

				52.85		100.3534

				52.87		100.3534

				52.89		100.3575

				52.91		100.3575

				52.93		100.3575

				52.95		100.3575

				52.97		100.3575

				52.99		100.3575

				53.01		100.3575

				53.03		100.3575

				53.05		100.3575

				53.07		100.3575

				53.09		100.3575

				53.11		100.3575

				53.13		100.3615

				53.15		100.3615

				53.17		100.3615

				53.19		100.3615

				53.21		100.3615

				53.23		100.3615

				53.25		100.3615

				53.27		100.3615

				53.29		100.3615

				53.31		100.3615

				53.33		100.3656

				53.35		100.3656

				53.37		100.3656

				53.39		100.3656

				53.41		100.3656

				53.43		100.3656

				53.45		100.3656

				53.47		100.3656

				53.49		100.3656

				53.51		100.3656

				53.53		100.3656

				53.55		100.3656

				53.57		100.3656

				53.59		100.3696

				53.61		100.3696

				53.63		100.3696

				53.65		100.3696

				53.67		100.3696

				53.69		100.3696

				53.71		100.3696

				53.74		100.3737

				53.76		100.3737

				53.78		100.3737

				53.8		100.3737

				53.82		100.3737

				53.84		100.3737

				53.86		100.3737

				53.88		100.3737

				53.9		100.3737

				53.92		100.3737

				53.94		100.3737

				53.96		100.3737

				53.98		100.3737

				54		100.3737

				54.02		100.3778

				54.04		100.3737

				54.06		100.3778

				54.08		100.3778

				54.1		100.3778

				54.12		100.3778

				54.14		100.3778

				54.16		100.3778

				54.18		100.3778

				54.2		100.3778

				54.22		100.3778

				54.24		100.3778

				54.26		100.3778

				54.28		100.3778

				54.3		100.3818

				54.32		100.3778

				54.34		100.3818

				54.36		100.3818

				54.38		100.3818

				54.41		100.3818

				54.43		100.3818

				54.45		100.3818

				54.47		100.3818

				54.49		100.3818

				54.51		100.3818

				54.53		100.3818

				54.55		100.3818

				54.57		100.3818

				54.59		100.3818

				54.61		100.3818

				54.63		100.3818

				54.65		100.3818

				54.67		100.3818

				54.69		100.3818

				54.71		100.3818

				54.73		100.3818

				54.75		100.3818

				54.77		100.3818

				54.79		100.3818

				54.81		100.3818

				54.83		100.3818

				54.85		100.3818

				54.87		100.3818

				54.89		100.3818

				54.91		100.3859

				54.93		100.3859

				54.95		100.3859

				54.97		100.3859

				55		100.3859

				55.02		100.3859

				55.04		100.3859

				55.06		100.3859

				55.08		100.3859

				55.1		100.3859

				55.12		100.3859

				55.14		100.3859

				55.16		100.3859

				55.18		100.3859

				55.2		100.3859

				55.22		100.3859

				55.24		100.3859

				55.26		100.3859

				55.28		100.3859

				55.3		100.3859

				55.32		100.3859

				55.34		100.3859

				55.36		100.39

				55.38		100.39

				55.4		100.39

				55.42		100.39

				55.44		100.39

				55.46		100.39

				55.48		100.39

				55.51		100.39

				55.53		100.39

				55.55		100.39

				55.57		100.39

				55.59		100.39

				55.61		100.39

				55.63		100.39

				55.65		100.39

				55.67		100.39

				55.69		100.39

				55.71		100.39

				55.73		100.39

				55.75		100.39

				55.77		100.39

				55.79		100.39

				55.81		100.39

				55.83		100.39

				55.85		100.39

				55.87		100.39

				55.89		100.39

				55.91		100.39

				55.93		100.394

				55.95		100.394

				55.97		100.39

				56		100.394

				56.02		100.394

				56.04		100.394

				56.06		100.394

				56.08		100.394

				56.1		100.394

				56.12		100.394

				56.14		100.394

				56.16		100.394

				56.18		100.394

				56.2		100.394

				56.22		100.394

				56.24		100.394

				56.26		100.394

				56.28		100.394

				56.3		100.394

				56.32		100.394

				56.34		100.394

				56.36		100.394

				56.38		100.394

				56.4		100.394

				56.42		100.394

				56.45		100.394

				56.47		100.394

				56.49		100.394

				56.51		100.394

				56.53		100.394

				56.55		100.394

				56.57		100.394

				56.59		100.394

				56.61		100.394

				56.63		100.394

				56.65		100.394

				56.67		100.3981

				56.69		100.3981

				56.71		100.3981

				56.73		100.3981

				56.75		100.3981

				56.77		100.3981

				56.79		100.3981

				56.81		100.3981

				56.83		100.3981

				56.85		100.3981

				56.88		100.3981

				56.9		100.3981

				56.92		100.3981

				56.94		100.3981

				56.96		100.3981

				56.98		100.3981

				57		100.3981

				57.02		100.3981

				57.04		100.3981

				57.06		100.3981

				57.08		100.3981

				57.1		100.3981

				57.12		100.3981

				57.14		100.3981

				57.16		100.3981

				57.18		100.3981

				57.2		100.3981

				57.22		100.3981

				57.24		100.3981

				57.27		100.3981

				57.29		100.3981

				57.31		100.3981

				57.33		100.3981

				57.35		100.3981

				57.37		100.3981

				57.39		100.3981

				57.41		100.3981

				57.43		100.3981

				57.45		100.3981

				57.47		100.3981

				57.49		100.3981

				57.51		100.4021

				57.53		100.4021

				57.55		100.4021

				57.57		100.4021

				57.59		100.4021

				57.61		100.4021

				57.64		100.4021

				57.66		100.4021

				57.68		100.4021

				57.7		100.4021

				57.72		100.4021

				57.74		100.4021

				57.76		100.4021

				57.78		100.4021

				57.8		100.4021

				57.82		100.4021

				57.84		100.4021

				57.86		100.4021

				57.88		100.4021

				57.9		100.4021

				57.92		100.4062

				57.94		100.4062

				57.96		100.4062

				57.98		100.4062

				58.01		100.4062

				58.03		100.4062

				58.05		100.4062

				58.07		100.4062

				58.09		100.4062

				58.11		100.4062

				58.13		100.4062

				58.15		100.4062

				58.17		100.4062

				58.19		100.4062

				58.21		100.4062

				58.23		100.4062

				58.25		100.4062

				58.27		100.4062

				58.29		100.4062

				58.31		100.4062

				58.33		100.4062

				58.35		100.4062

				58.38		100.4062

				58.4		100.4062

				58.42		100.4062

				58.44		100.4062

				58.46		100.4062

				58.48		100.4062

				58.5		100.4103

				58.52		100.4103

				58.54		100.4103

				58.56		100.4103

				58.58		100.4103

				58.6		100.4103

				58.62		100.4103

				58.64		100.4103

				58.66		100.4103

				58.68		100.4103

				58.7		100.4103

				58.73		100.4103

				58.75		100.4103

				58.77		100.4103

				58.79		100.4103

				58.81		100.4103

				58.83		100.4103

				58.85		100.4143

				58.87		100.4143

				58.89		100.4143

				58.91		100.4143

				58.93		100.4143

				58.95		100.4143

				58.97		100.4143

				58.99		100.4143

				59.01		100.4143

				59.03		100.4143

				59.06		100.4143

				59.08		100.4143

				59.1		100.4143

				59.12		100.4143

				59.14		100.4143

				59.16		100.4184

				59.18		100.4184

				59.2		100.4184

				59.22		100.4184

				59.24		100.4184

				59.26		100.4184

				59.28		100.4184

				59.3		100.4184

				59.32		100.4184

				59.34		100.4184

				59.36		100.4184

				59.38		100.4184

				59.41		100.4184

				59.43		100.4184

				59.45		100.4184

				59.47		100.4184

				59.49		100.4184

				59.51		100.4184

				59.53		100.4184

				59.55		100.4184

				59.57		100.4184

				59.59		100.4184

				59.61		100.4184

				59.63		100.4184

				59.65		100.4184

				59.67		100.4184

				59.69		100.4184

				59.71		100.4225

				59.74		100.4225

				59.76		100.4225

				59.78		100.4225

				59.8		100.4225

				59.82		100.4225

				59.84		100.4225

				59.86		100.4225

				59.88		100.4225

				59.9		100.4225

				59.92		100.4225

				59.94		100.4225

				59.96		100.4225

				59.98		100.4225

				60		100.4225

				60.02		100.4265

				60.04		100.4265

				60.06		100.4265

				60.09		100.4265

				60.11		100.4265

				60.13		100.4265

				60.15		100.4265

				60.17		100.4265

				60.19		100.4265

				60.21		100.4265

				60.23		100.4265

				60.25		100.4265

				60.27		100.4265

				60.29		100.4265

				60.31		100.4265

				60.33		100.4265

				60.35		100.4265

				60.37		100.4265

				60.39		100.4306

				60.42		100.4306

				60.44		100.4306

				60.46		100.4306

				60.48		100.4306

				60.5		100.4306

				60.52		100.4306

				60.54		100.4306

				60.56		100.4306

				60.58		100.4306

				60.6		100.4306

				60.62		100.4306

				60.64		100.4306

				60.66		100.4306

				60.68		100.4346

				60.7		100.4346

				60.72		100.4346

				60.75		100.4346

				60.77		100.4346

				60.79		100.4346

				60.81		100.4346

				60.83		100.4346

				60.85		100.4346

				60.87		100.4346

				60.89		100.4346

				60.91		100.4346

				60.93		100.4346

				60.95		100.4346

				60.97		100.4346

				60.99		100.4346

				61.01		100.4346

				61.03		100.4346

				61.05		100.4346

				61.07		100.4346

				61.1		100.4346

				61.12		100.4346

				61.14		100.4387

				61.16		100.4387

				61.18		100.4387

				61.2		100.4387

				61.22		100.4387

				61.24		100.4387

				61.26		100.4387

				61.28		100.4387

				61.3		100.4387

				61.32		100.4387

				61.34		100.4387

				61.36		100.4387

				61.38		100.4387

				61.4		100.4387

				61.42		100.4387

				61.45		100.4387

				61.47		100.4428

				61.49		100.4428

				61.51		100.4428

				61.53		100.4428

				61.55		100.4428

				61.57		100.4428

				61.59		100.4428

				61.61		100.4428

				61.63		100.4428

				61.65		100.4428

				61.67		100.4428

				61.69		100.4428

				61.71		100.4428

				61.73		100.4428

				61.75		100.4428

				61.77		100.4428

				61.79		100.4428

				61.82		100.4428

				61.84		100.4428

				61.86		100.4428

				61.88		100.4428

				61.9		100.4468

				61.92		100.4468

				61.94		100.4428

				61.96		100.4468

				61.98		100.4428

				62		100.4468

				62.02		100.4468

				62.04		100.4468

				62.06		100.4468

				62.08		100.4468

				62.1		100.4468

				62.12		100.4468

				62.14		100.4468

				62.17		100.4468

				62.19		100.4468

				62.21		100.4468

				62.23		100.4468

				62.25		100.4468

				62.27		100.4468

				62.29		100.4468

				62.31		100.4509

				62.33		100.4509

				62.35		100.4509

				62.37		100.4509

				62.39		100.4509

				62.41		100.4509

				62.43		100.4509

				62.45		100.4509

				62.47		100.4509

				62.49		100.4509

				62.51		100.4509

				62.54		100.4509

				62.56		100.4509

				62.58		100.4509

				62.6		100.4509

				62.62		100.4509

				62.64		100.4509

				62.66		100.4509

				62.68		100.4509

				62.7		100.4509

				62.72		100.4509

				62.74		100.4509

				62.76		100.4509

				62.78		100.4509

				62.8		100.4509

				62.82		100.4509

				62.84		100.4509

				62.86		100.4509

				62.88		100.4509

				62.9		100.4509

				62.93		100.4509

				62.95		100.4509

				62.97		100.455

				62.99		100.455

				63.01		100.455

				63.03		100.455

				63.05		100.455

				63.07		100.455

				63.09		100.455

				63.11		100.455

				63.13		100.455

				63.15		100.455

				63.17		100.455

				63.19		100.455

				63.21		100.455

				63.23		100.455

				63.25		100.455

				63.27		100.455

				63.29		100.455

				63.32		100.455

				63.34		100.455

				63.36		100.455

				63.38		100.455

				63.4		100.455

				63.42		100.455

				63.44		100.455

				63.46		100.455

				63.48		100.455

				63.5		100.455

				63.52		100.455

				63.54		100.455

				63.56		100.4509

				63.58		100.4509

				63.6		100.4509

				63.62		100.4509

				63.64		100.4509

				63.66		100.4509

				63.68		100.4509

				63.71		100.4509

				63.73		100.4509

				63.75		100.455

				63.77		100.455

				63.79		100.455

				63.81		100.455

				63.83		100.455

				63.85		100.455

				63.87		100.455

				63.89		100.455

				63.91		100.455

				63.93		100.4509

				63.95		100.455

				63.97		100.455

				63.99		100.4509

				64.01		100.455

				64.03		100.455

				64.05		100.455

				64.07		100.455

				64.09		100.455

				64.12		100.455

				64.14		100.455

				64.16		100.455

				64.18		100.455

				64.2		100.455

				64.22		100.455

				64.24		100.455

				64.26		100.455

				64.28		100.455

				64.3		100.455

				64.32		100.455

				64.34		100.455

				64.36		100.455

				64.38		100.455

				64.4		100.455

				64.42		100.455

				64.44		100.455

				64.46		100.455

				64.48		100.455

				64.51		100.455

				64.53		100.455

				64.55		100.455

				64.57		100.455

				64.59		100.455

				64.61		100.455

				64.63		100.455

				64.65		100.455

				64.67		100.455

				64.69		100.455

				64.71		100.455

				64.73		100.455

				64.75		100.455

				64.77		100.455

				64.79		100.455

				64.81		100.455

				64.83		100.455

				64.85		100.455

				64.87		100.455

				64.9		100.455

				64.92		100.455

				64.94		100.455

				64.96		100.455

				64.98		100.455

				65		100.455

				65.02		100.455

				65.04		100.459

				65.06		100.459

				65.08		100.459

				65.1		100.459

				65.12		100.459

				65.14		100.459

				65.16		100.459

				65.18		100.459

				65.2		100.459

				65.22		100.459

				65.24		100.459

				65.27		100.459

				65.29		100.459

				65.31		100.459

				65.33		100.459

				65.35		100.459

				65.37		100.459

				65.39		100.4631

				65.41		100.4631

				65.43		100.4631

				65.45		100.4631

				65.47		100.4631

				65.49		100.4631

				65.51		100.4631

				65.53		100.4631

				65.55		100.4631

				65.57		100.4631

				65.59		100.4631

				65.61		100.4631

				65.64		100.4631

				65.66		100.4631

				65.68		100.4631

				65.7		100.4631

				65.72		100.4631

				65.74		100.4631

				65.76		100.4631

				65.78		100.4631

				65.8		100.4631

				65.82		100.4631

				65.84		100.4631

				65.86		100.4631

				65.88		100.4631

				65.9		100.4631

				65.92		100.4631

				65.94		100.4631

				65.96		100.4671

				65.99		100.4631

				66.01		100.4631

				66.03		100.4631

				66.05		100.4631

				66.07		100.4631

				66.09		100.4631

				66.11		100.4631

				66.13		100.4631

				66.15		100.4631

				66.17		100.4631

				66.19		100.4631

				66.21		100.4631

				66.23		100.4631

				66.25		100.4631

				66.27		100.4631

				66.29		100.4631

				66.31		100.4631

				66.34		100.4631

				66.36		100.4631

				66.38		100.4631

				66.4		100.4631

				66.42		100.4631

				66.44		100.4671

				66.46		100.4631

				66.48		100.4631

				66.5		100.4671

				66.52		100.4671

				66.54		100.4671

				66.56		100.4671

				66.58		100.4671

				66.6		100.4671

				66.62		100.4671

				66.65		100.4671

				66.67		100.4671

				66.69		100.4671

				66.71		100.4671

				66.73		100.4671

				66.75		100.4671

				66.77		100.4671

				66.79		100.4671

				66.81		100.4671

				66.83		100.4671

				66.85		100.4671

				66.87		100.4671

				66.89		100.4671

				66.91		100.4671

				66.93		100.4671

				66.96		100.4671

				66.98		100.4671

				67		100.4671

				67.02		100.4671

				67.04		100.4671

				67.06		100.4671

				67.08		100.4671

				67.1		100.4671

				67.12		100.4671

				67.14		100.4671

				67.16		100.4671

				67.18		100.4671

				67.2		100.4671

				67.22		100.4671

				67.24		100.4671

				67.27		100.4671

				67.29		100.4671

				67.31		100.4671

				67.33		100.4671

				67.35		100.4671

				67.37		100.4631

				67.39		100.4631

				67.41		100.4631

				67.43		100.4631

				67.45		100.4631

				67.47		100.4631

				67.49		100.4631

				67.51		100.4631

				67.53		100.4631

				67.56		100.4671

				67.58		100.4631

				67.6		100.4671

				67.62		100.4671

				67.64		100.4671

				67.66		100.4671

				67.68		100.4671

				67.7		100.4671

				67.72		100.4671

				67.74		100.4671

				67.76		100.4671

				67.78		100.4671

				67.8		100.4631

				67.82		100.4631

				67.85		100.4631

				67.87		100.4631

				67.89		100.4631

				67.91		100.4631

				67.93		100.4631

				67.95		100.4631

				67.97		100.4671

				67.99		100.4631

				68.01		100.4631

				68.03		100.4631

				68.05		100.4631

				68.07		100.4631

				68.09		100.4671

				68.11		100.4631

				68.14		100.4631

				68.16		100.4631

				68.18		100.4631

				68.2		100.4671

				68.22		100.4671

				68.24		100.4671

				68.26		100.4671

				68.28		100.4671

				68.3		100.4631

				68.32		100.4671

				68.34		100.4671

				68.36		100.4671

				68.38		100.4671

				68.41		100.4671

				68.43		100.4671

				68.45		100.4671

				68.47		100.4631

				68.49		100.4631

				68.51		100.4671

				68.53		100.4631

				68.55		100.4631

				68.57		100.4631

				68.59		100.4631

				68.61		100.4631

				68.63		100.4631

				68.66		100.4631

				68.68		100.4631

				68.7		100.4631

				68.72		100.4631

				68.74		100.4631

				68.76		100.4631

				68.78		100.4631

				68.8		100.4631

				68.82		100.4631

				68.84		100.4631

				68.86		100.4631

				68.88		100.4671

				68.9		100.4671

				68.93		100.4671

				68.95		100.4671

				68.97		100.4671

				68.99		100.4671

				69.01		100.4671

				69.03		100.4671

				69.05		100.4671

				69.07		100.4631

				69.09		100.4631

				69.11		100.4631

				69.13		100.4671

				69.15		100.4671

				69.18		100.4671

				69.2		100.4671

				69.22		100.4671

				69.24		100.4671

				69.26		100.4671

				69.28		100.4671

				69.3		100.4671

				69.32		100.4671

				69.34		100.4671

				69.36		100.4671

				69.38		100.4671

				69.4		100.4671

				69.42		100.4671

				69.45		100.4671

				69.47		100.4671

				69.49		100.4671

				69.51		100.4671

				69.53		100.4671

				69.55		100.4671

				69.57		100.4671

				69.59		100.4671

				69.61		100.4671

				69.63		100.4671

				69.65		100.4712

				69.67		100.4671

				69.7		100.4712

				69.72		100.4712

				69.74		100.4712

				69.76		100.4712

				69.78		100.4712

				69.8		100.4712

				69.82		100.4712

				69.84		100.4712

				69.86		100.4712

				69.88		100.4712

				69.9		100.4712

				69.92		100.4712

				69.95		100.4712

				69.97		100.4712

				69.99		100.4712

				70.01		100.4712

				70.03		100.4712

				70.05		100.4712

				70.07		100.4712

				70.09		100.4712

				70.11		100.4712

				70.13		100.4712

				70.15		100.4712

				70.17		100.4712

				70.2		100.4712

				70.22		100.4712

				70.24		100.4712

				70.26		100.4712

				70.28		100.4712

				70.3		100.4712

				70.32		100.4712

				70.34		100.4712

				70.36		100.4712

				70.38		100.4712

				70.4		100.4712

				70.43		100.4712

				70.45		100.4712

				70.47		100.4712

				70.49		100.4712

				70.51		100.4712

				70.53		100.4712

				70.55		100.4712

				70.57		100.4712

				70.59		100.4712

				70.61		100.4712

				70.63		100.4712

				70.66		100.4712

				70.68		100.4712

				70.7		100.4712

				70.72		100.4712

				70.74		100.4712

				70.76		100.4712

				70.78		100.4712

				70.8		100.4712

				70.82		100.4712

				70.84		100.4712

				70.86		100.4712

				70.89		100.4712

				70.91		100.4712

				70.93		100.4712

				70.95		100.4712

				70.97		100.4712

				70.99		100.4712

				71.01		100.4712

				71.03		100.4712

				71.05		100.4712

				71.07		100.4712

				71.09		100.4712

				71.12		100.4712

				71.14		100.4712

				71.16		100.4712

				71.18		100.4712

				71.2		100.4712

				71.22		100.4712

				71.24		100.4712

				71.26		100.4712

				71.28		100.4712

				71.3		100.4712

				71.32		100.4712

				71.35		100.4712

				71.37		100.4712

				71.39		100.4712

				71.41		100.4712

				71.43		100.4712

				71.45		100.4712

				71.47		100.4753

				71.49		100.4753

				71.51		100.4753

				71.53		100.4753

				71.55		100.4753

				71.58		100.4753

				71.6		100.4753

				71.62		100.4753

				71.64		100.4753

				71.66		100.4753

				71.68		100.4753

				71.7		100.4712

				71.72		100.4712

				71.74		100.4712

				71.76		100.4712

				71.79		100.4712

				71.81		100.4753

				71.83		100.4753

				71.85		100.4753

				71.87		100.4753

				71.89		100.4753

				71.91		100.4753

				71.93		100.4753

				71.95		100.4753

				71.97		100.4753

				71.99		100.4753

				72.02		100.4753

				72.04		100.4753

				72.06		100.4753

				72.08		100.4753

				72.1		100.4753

				72.12		100.4753

				72.14		100.4753

				72.16		100.4753

				72.18		100.4753

				72.2		100.4753

				72.23		100.4753

				72.25		100.4753

				72.27		100.4753

				72.29		100.4753

				72.31		100.4753

				72.33		100.4753

				72.35		100.4753

				72.37		100.4753

				72.39		100.4793

				72.41		100.4793

				72.43		100.4793

				72.46		100.4793

				72.48		100.4793

				72.5		100.4793

				72.52		100.4793

				72.54		100.4793

				72.56		100.4793

				72.58		100.4793

				72.6		100.4793

				72.62		100.4793

				72.64		100.4793

				72.67		100.4793

				72.69		100.4793

				72.71		100.4793

				72.73		100.4793

				72.75		100.4793

				72.77		100.4793

				72.79		100.4793

				72.81		100.4834

				72.83		100.4834

				72.85		100.4834

				72.88		100.4834

				72.9		100.4834

				72.92		100.4834

				72.94		100.4834

				72.96		100.4834

				72.98		100.4834

				73		100.4834

				73.02		100.4834

				73.04		100.4834

				73.06		100.4834

				73.08		100.4834

				73.11		100.4834

				73.13		100.4834

				73.15		100.4834

				73.17		100.4834

				73.19		100.4834

				73.21		100.4834

				73.23		100.4834

				73.25		100.4874

				73.27		100.4874

				73.29		100.4874

				73.32		100.4874

				73.34		100.4874

				73.36		100.4874

				73.38		100.4874

				73.4		100.4874

				73.42		100.4874

				73.44		100.4874

				73.46		100.4874

				73.48		100.4874

				73.5		100.4874

				73.53		100.4874

				73.55		100.4874

				73.57		100.4874

				73.59		100.4874

				73.61		100.4874

				73.63		100.4874

				73.65		100.4874

				73.67		100.4874

				73.69		100.4874

				73.71		100.4874

				73.74		100.4915

				73.76		100.4915

				73.78		100.4915

				73.8		100.4915

				73.82		100.4915

				73.84		100.4915

				73.86		100.4915

				73.88		100.4915

				73.9		100.4915

				73.92		100.4915

				73.95		100.4915

				73.97		100.4915

				73.99		100.4915

				74.01		100.4915

				74.03		100.4915

				74.05		100.4915

				74.07		100.4915

				74.09		100.4956

				74.11		100.4956

				74.13		100.4956

				74.16		100.4956

				74.18		100.4956

				74.2		100.4956

				74.22		100.4956

				74.24		100.4956

				74.26		100.4956

				74.28		100.4956

				74.3		100.4956

				74.32		100.4956

				74.34		100.4956

				74.37		100.4996

				74.39		100.4996

				74.41		100.4996

				74.43		100.4996

				74.45		100.4996

				74.47		100.4996

				74.49		100.4996

				74.51		100.4996

				74.53		100.4996

				74.55		100.4996

				74.58		100.4996

				74.6		100.4996

				74.62		100.4996

				74.64		100.4996

				74.66		100.4996

				74.68		100.4996

				74.7		100.4996

				74.72		100.4996

				74.74		100.4996

				74.76		100.4996

				74.79		100.4996

				74.81		100.4996

				74.83		100.4996

				74.85		100.4996

				74.87		100.4996

				74.89		100.4996

				74.91		100.4996

				74.93		100.4996

				74.95		100.4996

				74.97		100.4996

				75		100.4996

				75.02		100.4996

				75.04		100.4996

				75.06		100.4996

				75.08		100.4996

				75.1		100.4996

				75.12		100.4996

				75.14		100.4996

				75.16		100.4996

				75.18		100.4996

				75.21		100.4996

				75.23		100.4996

				75.25		100.4996

				75.27		100.4996

				75.29		100.4996

				75.31		100.4996

				75.33		100.4996

				75.35		100.4996

				75.37		100.4996

				75.4		100.4996

				75.42		100.4996

				75.44		100.4996

				75.46		100.4996

				75.48		100.5037

				75.5		100.5037

				75.52		100.5037

				75.54		100.5037

				75.56		100.5037

				75.58		100.5037

				75.61		100.5037

				75.63		100.5037

				75.65		100.5037

				75.67		100.5037

				75.69		100.5037

				75.71		100.5037

				75.73		100.5037

				75.75		100.4996

				75.77		100.5037

				75.79		100.5037

				75.82		100.4996

				75.84		100.4996

				75.86		100.4996

				75.88		100.4996

				75.9		100.4996

				75.92		100.4996

				75.94		100.4996

				75.96		100.4996

				75.98		100.4996

				76.01		100.4996

				76.03		100.4996

				76.05		100.4996

				76.07		100.4996

				76.09		100.4996

				76.11		100.4996

				76.13		100.4996

				76.15		100.4996

				76.17		100.4996

				76.19		100.4996

				76.22		100.4996

				76.24		100.4996

				76.26		100.4996

				76.28		100.4996

				76.3		100.4996

				76.32		100.4996

				76.34		100.4996

				76.36		100.4996

				76.38		100.4996

				76.41		100.4996

				76.43		100.4996

				76.45		100.4996

				76.47		100.4996

				76.49		100.4996

				76.51		100.4996

				76.53		100.4996

				76.55		100.4996

				76.57		100.4996

				76.59		100.4996

				76.62		100.4996

				76.64		100.4996

				76.66		100.4996

				76.68		100.4996

				76.7		100.4996

				76.72		100.4996

				76.74		100.4996

				76.76		100.4996

				76.78		100.4996

				76.8		100.4996

				76.83		100.4996

				76.85		100.4996

				76.87		100.4996

				76.89		100.4996

				76.91		100.4996

				76.93		100.5037

				76.95		100.4996

				76.97		100.4996

				76.99		100.4996

				77.02		100.4996

				77.04		100.4996

				77.06		100.5037

				77.08		100.5037

				77.1		100.5037

				77.12		100.5037

				77.14		100.5037

				77.16		100.5037

				77.18		100.5037

				77.2		100.5037

				77.23		100.5037

				77.25		100.5037

				77.27		100.5037

				77.29		100.5037

				77.31		100.5037

				77.33		100.5037

				77.35		100.5037

				77.37		100.5037

				77.39		100.5037

				77.42		100.5037

				77.44		100.5037

				77.46		100.5037

				77.48		100.5037

				77.5		100.5037

				77.52		100.5037

				77.54		100.5037

				77.56		100.5037

				77.58		100.5037

				77.6		100.5037

				77.63		100.5037

				77.65		100.5037

				77.67		100.5037

				77.69		100.5037

				77.71		100.5037

				77.73		100.5037

				77.75		100.5037

				77.77		100.5037

				77.79		100.5037

				77.82		100.5037

				77.84		100.5037

				77.86		100.5037

				77.88		100.5037

				77.9		100.5037

				77.92		100.5078

				77.94		100.5078

				77.96		100.5078

				77.98		100.5037

				78		100.5037

				78.03		100.5037

				78.05		100.5037

				78.07		100.5037

				78.09		100.5037

				78.11		100.5037

				78.13		100.5037

				78.15		100.5037

				78.17		100.5078

				78.19		100.5078

				78.22		100.5078

				78.24		100.5078

				78.26		100.5078

				78.28		100.5078

				78.3		100.5078

				78.32		100.5078

				78.34		100.5078

				78.36		100.5037

				78.38		100.5037

				78.41		100.5037

				78.43		100.5037

				78.45		100.5037

				78.47		100.5037

				78.49		100.5037

				78.51		100.5037

				78.53		100.5037

				78.55		100.5037

				78.57		100.5037

				78.59		100.5037

				78.62		100.5037

				78.64		100.5037

				78.66		100.5037

				78.68		100.5078

				78.7		100.5078

				78.72		100.5037

				78.74		100.5078

				78.76		100.5078

				78.78		100.5078

				78.81		100.5078

				78.83		100.5078

				78.85		100.5078

				78.87		100.5078

				78.89		100.5078

				78.91		100.5078

				78.93		100.5078

				78.95		100.5078

				78.97		100.5078

				79		100.5078

				79.02		100.5078

				79.04		100.5078

				79.06		100.5078

				79.08		100.5078

				79.1		100.5078

				79.12		100.5078

				79.14		100.5078

				79.16		100.5078

				79.19		100.5078

				79.21		100.5078

				79.23		100.5078

				79.25		100.5078

				79.27		100.5078

				79.29		100.5078

				79.31		100.5118

				79.33		100.5078

				79.35		100.5118

				79.38		100.5118

				79.4		100.5118

				79.42		100.5118

				79.44		100.5078

				79.46		100.5118

				79.48		100.5118

				79.5		100.5118

				79.52		100.5118

				79.54		100.5118

				79.57		100.5118

				79.59		100.5118

				79.61		100.5118

				79.63		100.5118

				79.65		100.5078

				79.67		100.5118

				79.69		100.5118

				79.71		100.5118

				79.73		100.5118

				79.76		100.5118

				79.78		100.5118

				79.8		100.5118

				79.82		100.5118

				79.84		100.5118

				79.86		100.5118

				79.88		100.5118

				79.9		100.5118

				79.92		100.5118

				79.95		100.5118

				79.97		100.5118

				79.99		100.5118

				80.01		100.5118

				80.03		100.5118

				80.05		100.5118

				80.07		100.5118

				80.09		100.5118

				80.11		100.5118

				80.14		100.5118

				80.16		100.5118

				80.18		100.5118

				80.2		100.5118

				80.22		100.5118

				80.24		100.5118

				80.26		100.5118

				80.28		100.5118

				80.3		100.5118

				80.33		100.5118

				80.35		100.5118

				80.37		100.5159

				80.39		100.5159

				80.41		100.5118

				80.43		100.5159

				80.45		100.5159

				80.47		100.5159

				80.49		100.5159

				80.52		100.5159

				80.54		100.5159

				80.56		100.5159

				80.58		100.5159

				80.6		100.5159

				80.62		100.5159

				80.64		100.5118

				80.66		100.5159

				80.68		100.5159

				80.71		100.5118

				80.73		100.5159

				80.75		100.5159

				80.77		100.5159

				80.79		100.5118

				80.81		100.5159

				80.83		100.5159

				80.85		100.5159

				80.87		100.5159

				80.9		100.5159

				80.92		100.5118

				80.94		100.5118

				80.96		100.5159

				80.98		100.5159

				81		100.5159

				81.02		100.5159

				81.04		100.5159

				81.06		100.5159

				81.09		100.5159

				81.11		100.5159

				81.13		100.5159

				81.15		100.5159

				81.17		100.5159

				81.19		100.5159

				81.21		100.5159

				81.23		100.5159

				81.25		100.5159

				81.28		100.5159

				81.3		100.5159

				81.32		100.5159

				81.34		100.5159

				81.36		100.5159

				81.38		100.5159

				81.4		100.5159

				81.42		100.5159

				81.44		100.5159

				81.47		100.5199

				81.49		100.5199

				81.51		100.5199

				81.53		100.5199

				81.55		100.5199

				81.57		100.5199

				81.59		100.5199

				81.61		100.5199

				81.63		100.5199

				81.66		100.5199

				81.68		100.5199

				81.7		100.5199

				81.72		100.5199

				81.74		100.5199

				81.76		100.5199

				81.78		100.5199

				81.8		100.5199

				81.82		100.5199

				81.85		100.5199

				81.87		100.5199

				81.89		100.5199

				81.91		100.5199

				81.93		100.5199

				81.95		100.524

				81.97		100.524

				81.99		100.524

				82.01		100.524

				82.04		100.524

				82.06		100.524

				82.08		100.524

				82.1		100.524

				82.12		100.524

				82.14		100.524

				82.16		100.524

				82.18		100.524

				82.2		100.524

				82.22		100.524

				82.25		100.524

				82.27		100.524

				82.29		100.524

				82.31		100.524

				82.33		100.524

				82.35		100.524

				82.37		100.524

				82.39		100.524

				82.41		100.524

				82.44		100.524

				82.46		100.524

				82.48		100.524

				82.5		100.524

				82.52		100.524

				82.54		100.524

				82.56		100.524

				82.58		100.524

				82.6		100.524

				82.63		100.524

				82.65		100.524

				82.67		100.5281

				82.69		100.5281

				82.71		100.5281

				82.73		100.5281

				82.75		100.5281

				82.77		100.5281

				82.79		100.5281

				82.82		100.5281

				82.84		100.5281

				82.86		100.5281

				82.88		100.5281

				82.9		100.5281

				82.92		100.5281

				82.94		100.5281

				82.96		100.5281

				82.98		100.5281

				83.01		100.5321

				83.03		100.5321

				83.05		100.5281

				83.07		100.5281

				83.09		100.5281

				83.11		100.5281

				83.13		100.5321

				83.15		100.5321

				83.17		100.5321

				83.19		100.5321

				83.22		100.5321

				83.24		100.5321

				83.26		100.5321

				83.28		100.5321

				83.3		100.5321

				83.32		100.5321

				83.34		100.5321

				83.36		100.5321

				83.38		100.5321

				83.41		100.5321

				83.43		100.5321

				83.45		100.5321

				83.47		100.5321

				83.49		100.5321

				83.51		100.5321

				83.53		100.5321

				83.55		100.5321

				83.57		100.5321

				83.6		100.5321

				83.62		100.5321

				83.64		100.5321

				83.66		100.5321

				83.68		100.5321

				83.7		100.5321

				83.72		100.5362

				83.74		100.5362

				83.76		100.5362

				83.79		100.5362

				83.81		100.5362

				83.83		100.5362

				83.85		100.5362

				83.87		100.5362

				83.89		100.5362

				83.91		100.5362

				83.93		100.5362

				83.95		100.5362

				83.98		100.5362

				84		100.5362

				84.02		100.5362

				84.04		100.5362

				84.06		100.5362

				84.08		100.5362

				84.1		100.5362

				84.12		100.5362

				84.14		100.5362

				84.17		100.5362

				84.19		100.5362

				84.21		100.5362

				84.23		100.5362

				84.25		100.5362

				84.27		100.5362

				84.29		100.5362

				84.31		100.5362

				84.33		100.5362

				84.36		100.5362

				84.38		100.5362

				84.4		100.5362

				84.42		100.5362

				84.44		100.5362

				84.46		100.5362

				84.48		100.5362

				84.5		100.5362

				84.52		100.5362

				84.55		100.5362

				84.57		100.5403

				84.59		100.5403

				84.61		100.5362

				84.63		100.5403

				84.65		100.5403

				84.67		100.5403

				84.69		100.5403

				84.71		100.5403

				84.74		100.5403

				84.76		100.5403

				84.78		100.5403

				84.8		100.5403

				84.82		100.5403

				84.84		100.5403

				84.86		100.5403

				84.88		100.5403

				84.9		100.5403

				84.93		100.5403

				84.95		100.5403

				84.97		100.5403

				84.99		100.5403

				85.01		100.5403

				85.03		100.5403

				85.05		100.5403

				85.07		100.5403

				85.09		100.5403

				85.12		100.5403

				85.14		100.5403

				85.16		100.5403

				85.18		100.5403

				85.2		100.5403

				85.22		100.5403

				85.24		100.5403

				85.26		100.5403

				85.28		100.5403

				85.31		100.5403

				85.33		100.5403

				85.35		100.5403

				85.37		100.5443

				85.39		100.5443

				85.41		100.5443

				85.43		100.5443

				85.45		100.5443

				85.48		100.5443

				85.5		100.5443

				85.52		100.5403

				85.54		100.5403

				85.56		100.5403

				85.58		100.5403

				85.6		100.5403

				85.62		100.5403

				85.64		100.5443

				85.67		100.5443

				85.69		100.5443

				85.71		100.5443

				85.73		100.5443

				85.75		100.5443

				85.77		100.5443

				85.79		100.5443

				85.81		100.5443

				85.83		100.5443

				85.86		100.5443

				85.88		100.5443

				85.9		100.5443

				85.92		100.5443

				85.94		100.5443

				85.96		100.5443

				85.98		100.5443

				86		100.5443

				86.02		100.5443

				86.05		100.5443

				86.07		100.5443

				86.09		100.5443

				86.11		100.5443

				86.13		100.5443

				86.15		100.5443

				86.17		100.5443

				86.19		100.5443

				86.21		100.5443

				86.24		100.5443

				86.26		100.5443

				86.28		100.5443

				86.3		100.5443

				86.32		100.5443

				86.34		100.5443

				86.36		100.5443

				86.38		100.5443

				86.4		100.5443

				86.43		100.5443

				86.45		100.5443

				86.47		100.5443

				86.49		100.5443

				86.51		100.5484

				86.53		100.5443

				86.55		100.5484

				86.57		100.5443

				86.59		100.5443

				86.62		100.5443

				86.64		100.5484

				86.66		100.5484

				86.68		100.5484

				86.7		100.5484

				86.72		100.5484

				86.74		100.5484

				86.76		100.5484

				86.78		100.5484

				86.81		100.5484

				86.83		100.5484

				86.85		100.5484

				86.87		100.5484

				86.89		100.5484

				86.91		100.5484

				86.93		100.5484

				86.95		100.5484

				86.97		100.5484

				87		100.5484

				87.02		100.5484

				87.04		100.5484

				87.06		100.5484

				87.08		100.5484

				87.1		100.5484

				87.12		100.5484

				87.14		100.5484

				87.16		100.5484

				87.19		100.5484

				87.21		100.5484

				87.23		100.5484

				87.25		100.5484

				87.27		100.5484

				87.29		100.5484

				87.31		100.5484

				87.33		100.5484

				87.35		100.5484

				87.38		100.5484

				87.4		100.5484

				87.42		100.5484

				87.44		100.5484

				87.46		100.5484

				87.48		100.5484

				87.5		100.5484

				87.52		100.5484

				87.54		100.5484

				87.57		100.5484

				87.59		100.5484

				87.61		100.5484

				87.63		100.5484

				87.65		100.5484

				87.67		100.5484

				87.69		100.5484

				87.71		100.5484

				87.73		100.5484

				87.76		100.5484

				87.78		100.5484

				87.8		100.5484

				87.82		100.5484

				87.84		100.5484

				87.86		100.5484

				87.88		100.5484

				87.9		100.5484

				87.92		100.5484

				87.95		100.5484

				87.97		100.5524

				87.99		100.5524

				88.01		100.5524

				88.03		100.5524

				88.05		100.5524

				88.07		100.5524

				88.09		100.5524

				88.11		100.5524

				88.14		100.5524

				88.16		100.5524

				88.18		100.5524

				88.2		100.5565

				88.22		100.5565

				88.24		100.5565

				88.26		100.5565

				88.28		100.5565

				88.3		100.5565

				88.33		100.5565

				88.35		100.5565

				88.37		100.5565

				88.39		100.5565

				88.41		100.5565

				88.43		100.5565

				88.45		100.5565

				88.47		100.5565

				88.49		100.5565

				88.52		100.5565

				88.54		100.5565

				88.56		100.5565

				88.58		100.5565

				88.6		100.5565

				88.62		100.5565

				88.64		100.5565

				88.66		100.5565

				88.68		100.5565

				88.71		100.5565

				88.73		100.5565

				88.75		100.5565

				88.77		100.5565

				88.79		100.5565

				88.81		100.5565

				88.83		100.5565

				88.85		100.5565

				88.87		100.5565

				88.9		100.5565

				88.92		100.5565

				88.94		100.5565

				88.96		100.5565

				88.98		100.5565

				89		100.5565

				89.02		100.5565

				89.04		100.5565

				89.06		100.5565

				89.09		100.5565

				89.11		100.5565

				89.13		100.5565

				89.15		100.5565

				89.17		100.5565

				89.19		100.5565

				89.21		100.5565

				89.23		100.5565

				89.25		100.5565

				89.28		100.5565

				89.3		100.5606

				89.32		100.5565

				89.34		100.5606

				89.36		100.5606

				89.38		100.5606

				89.4		100.5606

				89.42		100.5606

				89.44		100.5606

				89.47		100.5606

				89.49		100.5606

				89.51		100.5606

				89.53		100.5606

				89.55		100.5606

				89.57		100.5606

				89.59		100.5606

				89.61		100.5606

				89.63		100.5606

				89.66		100.5606

				89.68		100.5606

				89.7		100.5646

				89.72		100.5646

				89.74		100.5646

				89.76		100.5646

				89.78		100.5646

				89.8		100.5646

				89.82		100.5646

				89.85		100.5646

				89.87		100.5646

				89.89		100.5646

				89.91		100.5646

				89.93		100.5646

				89.95		100.5646

				89.97		100.5646

				89.99		100.5646

				90.01		100.5646

				90.04		100.5646

				90.06		100.5646

				90.08		100.5646

				90.1		100.5646

				90.12		100.5646

				90.14		100.5646

				90.16		100.5646

				90.18		100.5646

				90.2		100.5646

				90.23		100.5646

				90.25		100.5646

				90.27		100.5646

				90.29		100.5646

				90.31		100.5646

				90.33		100.5646

				90.35		100.5646

				90.37		100.5646

				90.39		100.5646

				90.42		100.5646

				90.44		100.5646

				90.46		100.5646

				90.48		100.5646

				90.5		100.5646

				90.52		100.5646

				90.54		100.5646

				90.56		100.5646

				90.58		100.5646

				90.61		100.5646

				90.63		100.5646

				90.65		100.5646

				90.67		100.5646

				90.69		100.5646

				90.71		100.5646

				90.73		100.5646

				90.75		100.5646

				90.77		100.5646

				90.8		100.5646

				90.82		100.5646

				90.84		100.5646

				90.86		100.5646

				90.88		100.5646

				90.9		100.5646

				90.92		100.5646

				90.94		100.5646

				90.96		100.5646

				90.99		100.5646

				91.01		100.5646

				91.03		100.5687

				91.05		100.5687

				91.07		100.5646

				91.09		100.5687

				91.11		100.5687

				91.13		100.5687

				91.15		100.5687

				91.18		100.5687

				91.2		100.5687

				91.22		100.5687

				91.24		100.5687

				91.26		100.5687

				91.28		100.5687

				91.3		100.5687

				91.32		100.5687

				91.34		100.5687

				91.37		100.5687

				91.39		100.5687

				91.41		100.5687

				91.43		100.5687

				91.45		100.5687

				91.47		100.5687

				91.49		100.5687

				91.51		100.5687

				91.53		100.5646

				91.56		100.5687

				91.58		100.5687

				91.6		100.5687

				91.62		100.5687

				91.64		100.5687

				91.66		100.5687

				91.68		100.5687

				91.7		100.5687

				91.72		100.5687

				91.75		100.5687

				91.77		100.5687

				91.79		100.5646

				91.81		100.5646

				91.83		100.5646

				91.85		100.5646

				91.87		100.5646

				91.89		100.5646

				91.91		100.5646

				91.94		100.5646

				91.96		100.5646

				91.98		100.5646

				92		100.5646

				92.02		100.5646

				92.04		100.5646

				92.06		100.5646

				92.08		100.5646

				92.1		100.5646

				92.13		100.5646

				92.15		100.5646

				92.17		100.5646

				92.19		100.5646

				92.21		100.5646

				92.23		100.5646

				92.25		100.5646

				92.27		100.5646

				92.29		100.5646

				92.31		100.5646

				92.34		100.5646

				92.36		100.5646

				92.38		100.5646

				92.4		100.5687

				92.42		100.5687

				92.44		100.5687

				92.46		100.5687

				92.48		100.5687

				92.5		100.5687

				92.53		100.5687

				92.55		100.5687

				92.57		100.5687

				92.59		100.5687

				92.61		100.5687

				92.63		100.5687

				92.65		100.5687

				92.67		100.5687

				92.69		100.5687

				92.72		100.5687

				92.74		100.5687

				92.76		100.5646

				92.78		100.5646

				92.8		100.5687

				92.82		100.5687

				92.84		100.5687

				92.86		100.5687

				92.88		100.5687

				92.91		100.5687

				92.93		100.5687

				92.95		100.5687

				92.97		100.5687

				92.99		100.5646

				93.01		100.5646

				93.03		100.5687

				93.05		100.5687

				93.07		100.5687

				93.1		100.5687

				93.12		100.5646

				93.14		100.5687

				93.16		100.5646

				93.18		100.5646

				93.2		100.5646

				93.22		100.5646

				93.24		100.5646

				93.26		100.5646

				93.29		100.5646

				93.31		100.5646

				93.33		100.5646

				93.35		100.5646

				93.37		100.5646

				93.39		100.5646

				93.41		100.5646

				93.43		100.5646

				93.45		100.5646

				93.48		100.5646

				93.5		100.5646

				93.52		100.5646

				93.54		100.5646

				93.56		100.5646

				93.58		100.5646

				93.6		100.5646

				93.62		100.5646

				93.64		100.5646

				93.67		100.5646

				93.69		100.5646

				93.71		100.5646

				93.73		100.5646

				93.75		100.5646

				93.77		100.5646

				93.79		100.5646

				93.81		100.5646

				93.83		100.5646

				93.86		100.5646

				93.88		100.5646

				93.9		100.5646

				93.92		100.5646

				93.94		100.5646

				93.96		100.5646

				93.98		100.5646

				94		100.5646

				94.02		100.5646

				94.04		100.5646

				94.07		100.5646

				94.09		100.5646

				94.11		100.5646

				94.13		100.5646

				94.15		100.5646

				94.17		100.5646

				94.19		100.5646

				94.21		100.5646

				94.24		100.5646

				94.26		100.5646

				94.28		100.5646

				94.3		100.5687

				94.32		100.5687

				94.34		100.5687

				94.36		100.5687

				94.38		100.5646

				94.4		100.5646

				94.43		100.5646

				94.45		100.5646

				94.47		100.5646

				94.49		100.5646

				94.51		100.5646

				94.53		100.5646

				94.55		100.5646

				94.57		100.5646

				94.59		100.5646

				94.62		100.5646

				94.64		100.5646

				94.66		100.5646

				94.68		100.5646

				94.7		100.5646

				94.72		100.5646

				94.74		100.5687

				94.76		100.5687

				94.78		100.5687

				94.81		100.5687

				94.83		100.5687

				94.85		100.5687

				94.87		100.5687

				94.89		100.5687

				94.91		100.5687

				94.93		100.5687

				94.95		100.5687

				94.97		100.5687

				95		100.5687

				95.02		100.5687

				95.04		100.5687

				95.06		100.5687

				95.08		100.5687

				95.1		100.5687

				95.12		100.5687

				95.14		100.5687

				95.16		100.5687

				95.19		100.5687

				95.21		100.5687

				95.23		100.5687

				95.25		100.5687

				95.27		100.5687

				95.29		100.5687

				95.31		100.5687

				95.33		100.5728

				95.35		100.5728

				95.38		100.5728

				95.4		100.5728

				95.42		100.5728

				95.44		100.5728

				95.46		100.5728

				95.48		100.5728

				95.5		100.5728

				95.52		100.5728

				95.54		100.5728

				95.57		100.5728

				95.59		100.5728

				95.61		100.5728

				95.63		100.5728

				95.65		100.5728

				95.67		100.5768

				95.69		100.5728

				95.71		100.5768

				95.73		100.5768

				95.76		100.5728

				95.78		100.5728

				95.8		100.5768

				95.82		100.5728

				95.84		100.5768

				95.86		100.5728

				95.88		100.5728

				95.9		100.5728

				95.92		100.5768

				95.95		100.5728

				95.97		100.5728

				95.99		100.5728

				96.01		100.5728

				96.03		100.5768

				96.05		100.5768

				96.07		100.5768

				96.09		100.5768

				96.11		100.5728

				96.13		100.5768

				96.16		100.5768

				96.18		100.5768

				96.2		100.5768

				96.22		100.5768

				96.24		100.5728

				96.26		100.5768

				96.28		100.5728

				96.3		100.5728

				96.32		100.5728

				96.35		100.5728

				96.37		100.5728

				96.39		100.5728

				96.41		100.5728

				96.43		100.5728

				96.45		100.5728

				96.47		100.5728

				96.49		100.5728

				96.51		100.5728

				96.54		100.5728

				96.56		100.5728

				96.58		100.5768

				96.6		100.5768

				96.62		100.5768

				96.64		100.5768

				96.66		100.5768

				96.68		100.5768

				96.7		100.5768

				96.73		100.5768

				96.75		100.5768

				96.77		100.5768

				96.79		100.5768

				96.81		100.5768

				96.83		100.5768

				96.85		100.5768

				96.87		100.5768

				96.89		100.5768

				96.92		100.5768

				96.94		100.5768

				96.96		100.5768

				96.98		100.5768

				97		100.5768

				97.02		100.5768

				97.04		100.5768

				97.06		100.5768

				97.08		100.5768

				97.1		100.5768

				97.13		100.5768

				97.15		100.5768

				97.17		100.5768

				97.19		100.5768

				97.21		100.5768

				97.23		100.5768

				97.25		100.5768

				97.27		100.5768

				97.29		100.5768

				97.32		100.5768

				97.34		100.5768

				97.36		100.5768

				97.38		100.5768

				97.4		100.5768

				97.42		100.5768

				97.44		100.5809

				97.46		100.5809

				97.48		100.5809

				97.51		100.5809

				97.53		100.5809

				97.55		100.5809

				97.57		100.5809

				97.59		100.5809

				97.61		100.5809

				97.63		100.5809

				97.65		100.5809

				97.67		100.5809

				97.7		100.5809

				97.72		100.5809

				97.74		100.5809

				97.76		100.5809

				97.78		100.5809

				97.8		100.5809

				97.82		100.5809

				97.84		100.5809

				97.86		100.5809

				97.89		100.5809

				97.91		100.5809

				97.93		100.5809

				97.95		100.5809

				97.97		100.5809

				97.99		100.5809

				98.01		100.5809

				98.03		100.5809

				98.05		100.5809

				98.08		100.5809

				98.1		100.5809

				98.12		100.5809

				98.14		100.5809

				98.16		100.5809

				98.18		100.5809

				98.2		100.5809

				98.22		100.5809

				98.24		100.5809

				98.27		100.5809

				98.29		100.5809

				98.31		100.5809

				98.33		100.5809

				98.35		100.5809

				98.37		100.5809

				98.39		100.5809

				98.41		100.5809

				98.43		100.5809

				98.46		100.5809

				98.48		100.5809

				98.5		100.5809

				98.52		100.5809

				98.54		100.5809

				98.56		100.5809

				98.58		100.5809

				98.6		100.5809

				98.62		100.5809

				98.64		100.5809

				98.67		100.5809

				98.69		100.5809

				98.71		100.5809

				98.73		100.5809

				98.75		100.5809

				98.77		100.5809

				98.79		100.5809

				98.81		100.5809

				98.83		100.5809

				98.86		100.5809

				98.88		100.5809

				98.9		100.5809

				98.92		100.5809

				98.94		100.5809

				98.96		100.5809

				98.98		100.5809

				99		100.5809

				99.02		100.5809

				99.05		100.5809

				99.07		100.5809

				99.09		100.5809

				99.11		100.5809

				99.13		100.5809

				99.15		100.5809

				99.17		100.5809

				99.19		100.5809

				99.21		100.5809

				99.24		100.5809

				99.26		100.5809

				99.28		100.5809

				99.3		100.5809

				99.32		100.5809

				99.34		100.5809

				99.36		100.5809

				99.38		100.5809

				99.4		100.5809

				99.43		100.5809

				99.45		100.5809

				99.47		100.5809

				99.49		100.5809

				99.51		100.5809

				99.53		100.5809

				99.55		100.5809

				99.57		100.5809

				99.59		100.5809

				99.61		100.5809

				99.64		100.5809

				99.66		100.5809

				99.68		100.5809

				99.7		100.5809

				99.72		100.5809

				99.74		100.5809

				99.76		100.5809

				99.78		100.5809

				99.8		100.5809

				99.83		100.5809

				99.85		100.5809

				99.87		100.5809

				99.89		100.5809

				99.91		100.5809

				99.93		100.5809

				99.95		100.5809

				99.97		100.5809

				99.99		100.5809

				100.02		100.5849

				100.04		100.5809

				100.06		100.5849

				100.08		100.5849

				100.1		100.5809

				100.12		100.5809

				100.14		100.5809

				100.16		100.5809

				100.18		100.5849

				100.21		100.5809

				100.23		100.5809

				100.25		100.5809

				100.27		100.5809

				100.29		100.5809

				100.31		100.5809

				100.33		100.5849

				100.35		100.5809

				100.37		100.5809

				100.39		100.5809

				100.42		100.5809

				100.44		100.5809

				100.46		100.5809

				100.48		100.5849

				100.5		100.5849

				100.52		100.5809

				100.54		100.5849

				100.56		100.5849

				100.58		100.5849

				100.61		100.5849

				100.63		100.5849

				100.65		100.5849

				100.67		100.5849

				100.69		100.5849

				100.71		100.5849

				100.73		100.5809

				100.75		100.5809

				100.77		100.5809

				100.8		100.5809

				100.82		100.5809

				100.84		100.5809

				100.86		100.5809

				100.88		100.5809

				100.9		100.5849

				100.92		100.5849

				100.94		100.5809

				100.96		100.5849

				100.98		100.5809

				101.01		100.5809

				101.03		100.5809

				101.05		100.5809

				101.07		100.5809

				101.09		100.5809

				101.11		100.5809

				101.13		100.5809

				101.15		100.5809

				101.17		100.5809

				101.2		100.5809

				101.22		100.5809

				101.24		100.5809

				101.26		100.5809

				101.28		100.5849

				101.3		100.5809

				101.32		100.5849

				101.34		100.5849

				101.36		100.5809

				101.38		100.5849

				101.41		100.5849

				101.43		100.5849

				101.45		100.5849

				101.47		100.5849

				101.49		100.5849

				101.51		100.5809

				101.53		100.5809

				101.55		100.5849

				101.57		100.5809

				101.6		100.5849

				101.62		100.5809

				101.64		100.5849

				101.66		100.5809

				101.68		100.5809

				101.7		100.5849

				101.72		100.5809

				101.74		100.5849

				101.76		100.5849

				101.79		100.5849

				101.81		100.5849

				101.83		100.5849

				101.85		100.5849

				101.87		100.5849

				101.89		100.5849

				101.91		100.5849

				101.93		100.5849

				101.95		100.5849

				101.98		100.5849

				102		100.5849

				102.02		100.5849

				102.04		100.5849

				102.06		100.5849

				102.08		100.5849

				102.1		100.5849

				102.12		100.5849

				102.14		100.5849

				102.17		100.5849

				102.19		100.5849

				102.21		100.5849

				102.23		100.5849

				102.25		100.5849

				102.27		100.5849

				102.29		100.5849

				102.31		100.5849

				102.33		100.5849

				102.36		100.5849

				102.38		100.5849

				102.4		100.5849

				102.42		100.5849

				102.44		100.5849

				102.46		100.5849

				102.48		100.589

				102.5		100.589

				102.52		100.589

				102.55		100.589

				102.57		100.589

				102.59		100.589

				102.61		100.589

				102.63		100.589

				102.65		100.589

				102.67		100.589

				102.69		100.589

				102.71		100.589

				102.73		100.589

				102.76		100.589

				102.78		100.5931

				102.8		100.5931

				102.82		100.5931

				102.84		100.5931

				102.86		100.5931

				102.88		100.5931

				102.9		100.5931

				102.92		100.5931

				102.95		100.5931

				102.97		100.5931

				102.99		100.5931

				103.01		100.5931

				103.03		100.5931

				103.05		100.5931

				103.07		100.5931

				103.09		100.5931

				103.11		100.5931

				103.14		100.5931

				103.16		100.5931

				103.18		100.5931

				103.2		100.5931

				103.22		100.5971

				103.24		100.5971

				103.26		100.5971

				103.28		100.5971

				103.3		100.5971

				103.33		100.5971

				103.35		100.5971

				103.37		100.5971

				103.39		100.5971

				103.41		100.5971

				103.43		100.5971

				103.45		100.5971

				103.47		100.5971

				103.49		100.5971

				103.51		100.5971

				103.54		100.5971

				103.56		100.5971

				103.58		100.5971

				103.6		100.5971

				103.62		100.5971

				103.64		100.5971

				103.66		100.5971

				103.68		100.5971

				103.7		100.5971

				103.73		100.5971

				103.75		100.5971

				103.77		100.5971

				103.79		100.5971

				103.81		100.5971

				103.83		100.5971

				103.85		100.6012

				103.87		100.6012

				103.89		100.5971

				103.92		100.6012

				103.94		100.6012

				103.96		100.6012

				103.98		100.6012

				104		100.6012

				104.02		100.6012

				104.04		100.6012

				104.06		100.6012

				104.08		100.6012

				104.11		100.6012

				104.13		100.6012

				104.15		100.6012

				104.17		100.6012

				104.19		100.6012

				104.21		100.6012

				104.23		100.6012

				104.25		100.6012

				104.27		100.6012

				104.29		100.6012

				104.32		100.6012

				104.34		100.6012

				104.36		100.6012

				104.38		100.6012

				104.4		100.6012

				104.42		100.6012

				104.44		100.6012

				104.46		100.6012

				104.48		100.6012

				104.51		100.6012

				104.53		100.6012

				104.55		100.6012

				104.57		100.6012

				104.59		100.6012

				104.61		100.6012

				104.63		100.6012

				104.65		100.6012

				104.67		100.6012

				104.69		100.6012

				104.72		100.6012

				104.74		100.6012

				104.76		100.6012

				104.78		100.6012

				104.8		100.6012

				104.82		100.6012

				104.84		100.6012

				104.86		100.6012

				104.88		100.6012

				104.91		100.6012

				104.93		100.6012

				104.95		100.6012

				104.97		100.6012

				104.99		100.6012

				105.01		100.6012

				105.03		100.6012

				105.05		100.6012

				105.07		100.6012

				105.09		100.6012

				105.12		100.6012

				105.14		100.6012

				105.16		100.6012

				105.18		100.6012

				105.2		100.6012

				105.22		100.6012

				105.24		100.6012

				105.26		100.6012

				105.28		100.6012

				105.31		100.6012

				105.33		100.6012

				105.35		100.6012

				105.37		100.6012

				105.39		100.6012

				105.41		100.6012

				105.43		100.6012

				105.45		100.6012

				105.47		100.6012

				105.49		100.6012

				105.52		100.6012

				105.54		100.6012

				105.56		100.6012

				105.58		100.6012

				105.6		100.6012

				105.62		100.6012

				105.64		100.6012

				105.66		100.6012

				105.68		100.6012

				105.71		100.6012

				105.73		100.6012

				105.75		100.6012

				105.77		100.6012

				105.79		100.6012

				105.81		100.6012

				105.83		100.6012

				105.85		100.6012

				105.87		100.6012

				105.9		100.6012

				105.92		100.6012

				105.94		100.6012

				105.96		100.6012

				105.98		100.6012

				106		100.6012

				106.02		100.6012

				106.04		100.6012

				106.06		100.6012

				106.08		100.6012

				106.11		100.6012

				106.13		100.6012

				106.15		100.6012

				106.17		100.6012

				106.19		100.6012

				106.21		100.6012

				106.23		100.6012

				106.25		100.6012

				106.27		100.6012

				106.3		100.6012

				106.32		100.6012

				106.34		100.6012

				106.36		100.6012

				106.38		100.6012

				106.4		100.6012

				106.42		100.6012

				106.44		100.6012

				106.46		100.6012

				106.49		100.6012

				106.51		100.6012

				106.53		100.6012

				106.55		100.6012

				106.57		100.6012

				106.59		100.6012

				106.61		100.6052

				106.63		100.6052

				106.65		100.6052

				106.67		100.6052

				106.7		100.6052

				106.72		100.6052

				106.74		100.6052

				106.76		100.6052

				106.78		100.6052

				106.8		100.6052

				106.82		100.6052

				106.84		100.6052

				106.86		100.6052

				106.89		100.6052

				106.91		100.6052

				106.93		100.6052

				106.95		100.6052

				106.97		100.6093

				106.99		100.6093

				107.01		100.6093

				107.03		100.6093

				107.05		100.6093

				107.07		100.6093

				107.1		100.6093

				107.12		100.6093

				107.14		100.6093

				107.16		100.6093

				107.18		100.6093

				107.2		100.6093

				107.22		100.6093

				107.24		100.6093

				107.26		100.6093

				107.29		100.6093

				107.31		100.6093

				107.33		100.6134

				107.35		100.6134

				107.37		100.6134

				107.39		100.6134

				107.41		100.6134

				107.43		100.6134

				107.45		100.6134

				107.47		100.6134

				107.5		100.6134

				107.52		100.6134

				107.54		100.6134

				107.56		100.6134

				107.58		100.6134

				107.6		100.6134

				107.62		100.6134

				107.64		100.6134

				107.66		100.6134

				107.69		100.6134

				107.71		100.6134

				107.73		100.6134

				107.75		100.6134

				107.77		100.6134

				107.79		100.6134

				107.81		100.6134

				107.83		100.6134

				107.85		100.6134

				107.88		100.6134

				107.9		100.6134

				107.92		100.6134

				107.94		100.6134

				107.96		100.6134

				107.98		100.6134

				108		100.6134

				108.02		100.6134

				108.04		100.6134

				108.07		100.6134

				108.09		100.6134

				108.11		100.6134

				108.13		100.6174

				108.15		100.6174

				108.17		100.6174

				108.19		100.6174

				108.21		100.6174

				108.23		100.6174

				108.25		100.6174

				108.28		100.6174

				108.3		100.6174

				108.32		100.6174

				108.34		100.6174

				108.36		100.6174

				108.38		100.6174

				108.4		100.6174

				108.42		100.6174

				108.44		100.6174

				108.47		100.6174

				108.49		100.6174

				108.51		100.6174

				108.53		100.6174

				108.55		100.6174

				108.57		100.6174

				108.59		100.6174

				108.61		100.6174

				108.63		100.6174

				108.65		100.6215

				108.68		100.6215

				108.7		100.6174

				108.72		100.6174

				108.74		100.6174

				108.76		100.6174

				108.78		100.6215

				108.8		100.6174

				108.82		100.6174

				108.84		100.6174

				108.87		100.6174

				108.89		100.6174

				108.91		100.6215

				108.93		100.6174

				108.95		100.6174

				108.97		100.6174

				108.99		100.6174

				109.01		100.6174

				109.03		100.6215

				109.06		100.6174

				109.08		100.6174

				109.1		100.6174

				109.12		100.6174

				109.14		100.6174

				109.16		100.6174

				109.18		100.6174

				109.2		100.6215

				109.22		100.6174

				109.24		100.6174

				109.27		100.6174

				109.29		100.6215

				109.31		100.6174

				109.33		100.6215

				109.35		100.6215

				109.37		100.6174

				109.39		100.6174

				109.41		100.6215

				109.43		100.6215

				109.46		100.6215

				109.48		100.6215

				109.5		100.6215

				109.52		100.6215

				109.54		100.6215

				109.56		100.6215

				109.58		100.6215

				109.6		100.6215

				109.62		100.6215

				109.64		100.6215

				109.67		100.6215

				109.69		100.6215

				109.71		100.6215

				109.73		100.6215

				109.75		100.6215

				109.77		100.6215

				109.79		100.6215

				109.81		100.6215

				109.83		100.6215

				109.86		100.6215

				109.88		100.6215

				109.9		100.6215

				109.92		100.6215

				109.94		100.6215

				109.96		100.6215

				109.98		100.6215

				110		100.6215

				110.02		100.6215

				110.05		100.6215

				110.07		100.6215

				110.09		100.6215

				110.11		100.6215

				110.13		100.6215

				110.15		100.6215

				110.17		100.6215

				110.19		100.6215

				110.21		100.6215

				110.23		100.6215

				110.26		100.6215

				110.28		100.6215

				110.3		100.6215

				110.32		100.6215

				110.34		100.6215

				110.36		100.6215

				110.38		100.6215

				110.4		100.6215

				110.42		100.6215

				110.45		100.6215

				110.47		100.6215

				110.49		100.6215

				110.51		100.6215

				110.53		100.6215

				110.55		100.6215

				110.57		100.6215

				110.59		100.6215

				110.61		100.6215

				110.64		100.6215

				110.66		100.6215

				110.68		100.6215

				110.7		100.6215

				110.72		100.6215

				110.74		100.6215

				110.76		100.6215

				110.78		100.6215

				110.8		100.6215

				110.83		100.6215

				110.85		100.6215

				110.87		100.6215

				110.89		100.6215

				110.91		100.6215

				110.93		100.6215

				110.95		100.6215

				110.97		100.6215

				110.99		100.6215

				111.01		100.6215

				111.04		100.6215

				111.06		100.6215

				111.08		100.6215

				111.1		100.6215

				111.12		100.6215

				111.14		100.6215

				111.16		100.6215

				111.18		100.6215

				111.2		100.6215

				111.23		100.6215

				111.25		100.6215

				111.27		100.6215

				111.29		100.6215

				111.31		100.6215

				111.33		100.6215

				111.35		100.6215

				111.37		100.6215

				111.39		100.6256

				111.41		100.6215

				111.44		100.6215

				111.46		100.6215

				111.48		100.6256

				111.5		100.6215

				111.52		100.6215

				111.54		100.6215

				111.56		100.6215

				111.58		100.6215

				111.6		100.6215

				111.63		100.6215

				111.65		100.6215

				111.67		100.6215

				111.69		100.6215

				111.71		100.6215

				111.73		100.6215

				111.75		100.6215

				111.77		100.6215

				111.79		100.6215

				111.81		100.6215

				111.84		100.6215

				111.86		100.6215

				111.88		100.6256

				111.9		100.6215

				111.92		100.6215

				111.94		100.6215

				111.96		100.6215

				111.98		100.6215

				112		100.6215

				112.03		100.6215

				112.05		100.6215

				112.07		100.6215

				112.09		100.6215

				112.11		100.6215

				112.13		100.6215

				112.15		100.6215

				112.17		100.6215

				112.19		100.6215

				112.21		100.6215

				112.24		100.6215

				112.26		100.6215

				112.28		100.6215

				112.3		100.6215

				112.32		100.6215

				112.34		100.6215

				112.36		100.6215

				112.38		100.6215

				112.4		100.6215

				112.43		100.6215

				112.45		100.6215

				112.47		100.6215

				112.49		100.6215

				112.51		100.6215

				112.53		100.6215

				112.55		100.6215

				112.57		100.6215

				112.59		100.6215

				112.61		100.6215

				112.64		100.6215

				112.66		100.6215

				112.68		100.6215

				112.7		100.6215

				112.72		100.6215

				112.74		100.6215

				112.76		100.6215

				112.78		100.6215

				112.8		100.6215

				112.83		100.6215

				112.85		100.6215

				112.87		100.6215

				112.89		100.6215

				112.91		100.6215

				112.93		100.6215

				112.95		100.6215

				112.97		100.6215

				112.99		100.6215

				113.01		100.6215

				113.04		100.6215

				113.06		100.6215

				113.08		100.6215

				113.1		100.6215

				113.12		100.6215

				113.14		100.6215

				113.16		100.6215

				113.18		100.6215

				113.2		100.6215

				113.23		100.6215

				113.25		100.6215

				113.27		100.6215

				113.29		100.6215

				113.31		100.6215

				113.33		100.6215

				113.35		100.6215

				113.37		100.6215

				113.39		100.6215

				113.42		100.6215

				113.44		100.6215

				113.46		100.6215

				113.48		100.6215

				113.5		100.6215

				113.52		100.6215

				113.54		100.6215

				113.56		100.6215

				113.58		100.6215

				113.6		100.6215

				113.63		100.6215

				113.65		100.6215

				113.67		100.6215

				113.69		100.6215

				113.71		100.6215

				113.73		100.6215

				113.75		100.6215

				113.77		100.6215

				113.79		100.6215

				113.82		100.6215

				113.84		100.6215

				113.86		100.6215

				113.88		100.6215

				113.9		100.6215

				113.92		100.6215

				113.94		100.6215

				113.96		100.6215

				113.98		100.6215

				114		100.6215

				114.03		100.6215

				114.05		100.6215

				114.07		100.6215

				114.09		100.6215

				114.11		100.6215

				114.13		100.6215

				114.15		100.6215

				114.17		100.6215

				114.19		100.6215

				114.22		100.6215

				114.24		100.6215

				114.26		100.6215

				114.28		100.6215

				114.3		100.6215

				114.32		100.6215

				114.34		100.6215

				114.36		100.6215

				114.38		100.6215

				114.41		100.6215

				114.43		100.6215

				114.45		100.6215

				114.47		100.6215

				114.49		100.6215

				114.51		100.6215

				114.53		100.6215

				114.55		100.6215

				114.57		100.6215

				114.59		100.6215

				114.62		100.6215

				114.64		100.6215

				114.66		100.6215

				114.68		100.6215

				114.7		100.6174

				114.72		100.6215

				114.74		100.6174

				114.76		100.6174

				114.78		100.6174

				114.81		100.6174

				114.83		100.6174

				114.85		100.6174

				114.87		100.6174

				114.89		100.6174

				114.91		100.6174

				114.93		100.6174

				114.95		100.6174

				114.97		100.6174

				115		100.6174

				115.02		100.6174

				115.04		100.6174

				115.06		100.6174

				115.08		100.6174

				115.1		100.6174

				115.12		100.6174

				115.14		100.6174

				115.16		100.6174

				115.18		100.6174

				115.21		100.6174

				115.23		100.6174

				115.25		100.6174

				115.27		100.6134

				115.29		100.6134

				115.31		100.6134

				115.33		100.6134

				115.35		100.6134

				115.37		100.6134

				115.4		100.6134

				115.42		100.6134

				115.44		100.6134

				115.46		100.6134

				115.48		100.6134

				115.5		100.6134

				115.52		100.6134

				115.54		100.6134

				115.56		100.6134

				115.59		100.6134

				115.61		100.6134

				115.63		100.6134

				115.65		100.6134

				115.67		100.6134

				115.69		100.6134

				115.71		100.6134

				115.73		100.6134

				115.75		100.6134

				115.77		100.6134

				115.8		100.6134

				115.82		100.6134

				115.84		100.6134

				115.86		100.6134

				115.88		100.6134

				115.9		100.6134

				115.92		100.6134

				115.94		100.6134

				115.96		100.6134

				115.99		100.6134

				116.01		100.6134

				116.03		100.6134

				116.05		100.6134

				116.07		100.6134

				116.09		100.6134

				116.11		100.6134

				116.13		100.6134

				116.15		100.6134

				116.17		100.6134

				116.2		100.6134

				116.22		100.6134

				116.24		100.6134

				116.26		100.6134

				116.28		100.6134

				116.3		100.6134

				116.32		100.6134

				116.34		100.6134

				116.36		100.6134

				116.39		100.6134

				116.41		100.6134

				116.43		100.6134

				116.45		100.6134

				116.47		100.6134

				116.49		100.6134

				116.51		100.6134

				116.53		100.6134

				116.55		100.6134

				116.58		100.6134

				116.6		100.6134

				116.62		100.6134

				116.64		100.6134

				116.66		100.6134

				116.68		100.6134

				116.7		100.6134

				116.72		100.6134

				116.74		100.6134

				116.76		100.6134

				116.79		100.6134

				116.81		100.6134

				116.83		100.6134

				116.85		100.6134

				116.87		100.6134

				116.89		100.6134

				116.91		100.6134

				116.93		100.6134

				116.95		100.6134

				116.98		100.6134

				117		100.6134

				117.02		100.6134

				117.04		100.6134

				117.06		100.6134

				117.08		100.6134

				117.1		100.6134

				117.12		100.6134

				117.14		100.6134

				117.16		100.6134

				117.19		100.6134

				117.21		100.6134

				117.23		100.6134

				117.25		100.6134

				117.27		100.6134

				117.29		100.6134

				117.31		100.6134

				117.33		100.6134

				117.35		100.6134

				117.38		100.6134

				117.4		100.6134

				117.42		100.6134

				117.44		100.6134

				117.46		100.6134

				117.48		100.6134

				117.5		100.6134

				117.52		100.6134

				117.54		100.6134

				117.57		100.6134

				117.59		100.6134

				117.61		100.6134

				117.63		100.6134

				117.65		100.6134

				117.67		100.6134

				117.69		100.6134

				117.71		100.6134

				117.73		100.6134

				117.75		100.6134

				117.78		100.6174

				117.8		100.6134

				117.82		100.6134

				117.84		100.6174

				117.86		100.6174

				117.88		100.6174

				117.9		100.6174

				117.92		100.6174

				117.94		100.6174

				117.97		100.6174

				117.99		100.6174

				118.01		100.6174

				118.03		100.6174

				118.05		100.6174

				118.07		100.6174

				118.09		100.6174

				118.11		100.6174

				118.13		100.6174

				118.15		100.6174

				118.18		100.6174

				118.2		100.6174

				118.22		100.6174

				118.24		100.6174

				118.26		100.6174

				118.28		100.6174

				118.3		100.6174

				118.32		100.6174

				118.34		100.6174

				118.37		100.6174

				118.39		100.6174

				118.41		100.6174

				118.43		100.6174

				118.45		100.6174

				118.47		100.6174

				118.49		100.6174

				118.51		100.6215

				118.53		100.6215

				118.55		100.6215

				118.58		100.6215

				118.6		100.6215

				118.62		100.6215

				118.64		100.6215

				118.66		100.6215

				118.68		100.6215

				118.7		100.6215

				118.72		100.6215

				118.74		100.6215

				118.77		100.6215

				118.79		100.6215

				118.81		100.6215

				118.83		100.6215

				118.85		100.6215

				118.87		100.6215

				118.89		100.6215

				118.91		100.6215

				118.93		100.6256

				118.95		100.6256

				118.98		100.6256

				119		100.6256

				119.02		100.6256

				119.04		100.6256

				119.06		100.6256

				119.08		100.6256

				119.1		100.6256

				119.12		100.6256

				119.14		100.6256

				119.16		100.6256

				119.19		100.6256

				119.21		100.6256

				119.23		100.6256

				119.25		100.6256

				119.27		100.6256

				119.29		100.6256

				119.31		100.6256

				119.33		100.6256

				119.35		100.6256

				119.38		100.6256

				119.4		100.6256

				119.42		100.6256

				119.44		100.6256

				119.46		100.6256

				119.48		100.6256

				119.5		100.6256

				119.52		100.6256

				119.54		100.6256

				119.56		100.6256

				119.59		100.6256

				119.61		100.6256

				119.63		100.6296

				119.65		100.6296

				119.67		100.6296

				119.69		100.6296

				119.71		100.6296

				119.73		100.6296

				119.75		100.6296

				119.77		100.6296

				119.8		100.6296

				119.82		100.6296

				119.84		100.6296

				119.86		100.6296

				119.88		100.6296

				119.9		100.6296

				119.92		100.6296

				119.94		100.6296

				119.96		100.6296

				119.99		100.6296

				120.01		100.6256

				120.03		100.6296

				120.05		100.6296

				120.07		100.6296

				120.09		100.6296

				120.11		100.6296

				120.13		100.6256

				120.15		100.6296

				120.18		100.6296

				120.2		100.6296

				120.22		100.6296

				120.24		100.6296

				120.26		100.6296

				120.28		100.6296

				120.3		100.6296

				120.32		100.6296

				120.34		100.6296

				120.36		100.6296

				120.39		100.6296

				120.41		100.6296

				120.43		100.6296

				120.45		100.6296

				120.47		100.6296

				120.49		100.6256

				120.51		100.6256

				120.53		100.6256

				120.55		100.6256

				120.58		100.6256

				120.6		100.6256

				120.62		100.6256

				120.64		100.6256

				120.66		100.6256

				120.68		100.6256

				120.7		100.6256

				120.72		100.6256

				120.74		100.6256

				120.76		100.6256

				120.79		100.6256

				120.81		100.6256

				120.83		100.6256

				120.85		100.6256

				120.87		100.6256

				120.89		100.6256

				120.91		100.6256

				120.93		100.6256

				120.95		100.6256

				120.97		100.6256

				121		100.6256

				121.02		100.6256

				121.04		100.6256

				121.06		100.6256

				121.08		100.6256

				121.1		100.6256

				121.12		100.6256

				121.14		100.6256

				121.16		100.6256

				121.19		100.6256

				121.21		100.6256

				121.23		100.6256

				121.25		100.6256

				121.27		100.6256

				121.29		100.6256

				121.31		100.6256

				121.33		100.6296

				121.35		100.6256

				121.37		100.6296

				121.4		100.6296

				121.42		100.6296

				121.44		100.6256

				121.46		100.6256

				121.48		100.6256

				121.5		100.6256

				121.52		100.6296

				121.54		100.6296

				121.56		100.6296

				121.59		100.6296

				121.61		100.6296

				121.63		100.6296

				121.65		100.6296

				121.67		100.6296

				121.69		100.6296

				121.71		100.6296

				121.73		100.6296

				121.75		100.6296

				121.77		100.6296

				121.8		100.6296

				121.82		100.6296

				121.84		100.6296

				121.86		100.6296

				121.88		100.6296

				121.9		100.6296

				121.92		100.6296

				121.94		100.6296

				121.96		100.6296

				121.99		100.6296

				122.01		100.6296

				122.03		100.6296

				122.05		100.6296

				122.07		100.6296

				122.09		100.6296

				122.11		100.6296

				122.13		100.6296

				122.15		100.6296

				122.18		100.6296

				122.2		100.6296

				122.22		100.6337

				122.24		100.6337

				122.26		100.6337

				122.28		100.6337

				122.3		100.6337

				122.32		100.6337

				122.34		100.6337

				122.36		100.6337

				122.39		100.6337

				122.41		100.6337

				122.43		100.6337

				122.45		100.6337

				122.47		100.6337

				122.49		100.6337

				122.51		100.6337

				122.53		100.6337

				122.55		100.6337

				122.57		100.6337

				122.6		100.6337

				122.62		100.6337

				122.64		100.6337

				122.66		100.6337

				122.68		100.6337

				122.7		100.6337

				122.72		100.6337

				122.74		100.6337

				122.76		100.6337

				122.79		100.6337

				122.81		100.6337

				122.83		100.6337

				122.85		100.6337

				122.87		100.6337

				122.89		100.6337

				122.91		100.6337

				122.93		100.6337

				122.95		100.6337

				122.98		100.6337

				123		100.6337

				123.02		100.6337

				123.04		100.6337

				123.06		100.6337

				123.08		100.6337

				123.1		100.6337

				123.12		100.6337

				123.14		100.6337

				123.16		100.6337

				123.19		100.6337

				123.21		100.6337

				123.23		100.6337

				123.25		100.6337

				123.27		100.6337

				123.29		100.6337

				123.31		100.6337

				123.33		100.6337

				123.35		100.6337

				123.38		100.6337

				123.4		100.6337

				123.42		100.6337

				123.44		100.6337

				123.46		100.6337

				123.48		100.6337

				123.5		100.6337

				123.52		100.6337

				123.54		100.6337

				123.56		100.6337

				123.59		100.6337

				123.61		100.6337

				123.63		100.6337

				123.65		100.6337

				123.67		100.6337

				123.69		100.6296

				123.71		100.6337

				123.73		100.6337

				123.75		100.6296

				123.78		100.6296

				123.8		100.6296

				123.82		100.6296

				123.84		100.6296

				123.86		100.6296

				123.88		100.6296

				123.9		100.6296

				123.92		100.6296

				123.94		100.6296

				123.97		100.6296

				123.99		100.6296

				124.01		100.6296

				124.03		100.6296

				124.05		100.6296

				124.07		100.6296

				124.09		100.6296

				124.11		100.6296

				124.13		100.6296

				124.16		100.6296

				124.18		100.6296

				124.2		100.6296

				124.22		100.6296

				124.24		100.6296

				124.26		100.6296

				124.28		100.6296

				124.3		100.6296

				124.32		100.6296

				124.35		100.6296

				124.37		100.6296

				124.39		100.6296

				124.41		100.6256

				124.43		100.6296

				124.45		100.6256

				124.47		100.6256

				124.49		100.6256

				124.51		100.6256

				124.54		100.6256

				124.56		100.6256

				124.58		100.6256

				124.6		100.6256

				124.62		100.6256

				124.64		100.6256

				124.66		100.6256

				124.68		100.6256

				124.7		100.6256

				124.72		100.6256

				124.75		100.6256

				124.77		100.6256

				124.79		100.6256

				124.81		100.6256

				124.83		100.6256

				124.85		100.6256

				124.87		100.6256

				124.89		100.6256

				124.91		100.6256

				124.94		100.6256

				124.96		100.6256

				124.98		100.6256

				125		100.6256

				125.02		100.6256

				125.04		100.6215

				125.06		100.6215

				125.08		100.6215

				125.1		100.6256

				125.13		100.6215

				125.15		100.6256

				125.17		100.6256

				125.19		100.6256

				125.21		100.6215

				125.23		100.6215

				125.25		100.6215

				125.27		100.6215

				125.29		100.6215

				125.32		100.6215

				125.34		100.6215

				125.36		100.6215

				125.38		100.6215

				125.4		100.6215

				125.42		100.6215

				125.44		100.6215

				125.46		100.6215

				125.48		100.6215

				125.51		100.6215

				125.53		100.6215

				125.55		100.6215

				125.57		100.6215

				125.59		100.6215

				125.61		100.6215

				125.63		100.6215

				125.65		100.6215

				125.67		100.6215

				125.7		100.6215

				125.72		100.6215

				125.74		100.6215

				125.76		100.6174

				125.78		100.6215

				125.8		100.6215

				125.82		100.6174

				125.84		100.6174

				125.86		100.6174

				125.89		100.6174

				125.91		100.6174

				125.93		100.6174

				125.95		100.6174

				125.97		100.6174

				125.99		100.6174

				126.01		100.6174

				126.03		100.6174

				126.05		100.6174

				126.08		100.6174

				126.1		100.6174

				126.12		100.6174

				126.14		100.6174

				126.16		100.6174

				126.18		100.6174

				126.2		100.6174

				126.22		100.6174

				126.24		100.6174

				126.27		100.6174

				126.29		100.6174

				126.31		100.6174

				126.33		100.6174

				126.35		100.6174

				126.37		100.6174

				126.39		100.6174

				126.41		100.6174

				126.43		100.6174

				126.46		100.6174

				126.48		100.6174

				126.5		100.6174

				126.52		100.6174

				126.54		100.6174

				126.56		100.6174

				126.58		100.6174

				126.6		100.6174

				126.62		100.6174

				126.65		100.6174

				126.67		100.6174

				126.69		100.6174

				126.71		100.6174

				126.73		100.6174

				126.75		100.6174

				126.77		100.6174

				126.79		100.6174

				126.81		100.6174

				126.84		100.6174

				126.86		100.6174

				126.88		100.6174

				126.9		100.6174

				126.92		100.6174

				126.94		100.6174

				126.96		100.6174

				126.98		100.6174

				127		100.6174

				127.03		100.6174

				127.05		100.6174

				127.07		100.6174

				127.09		100.6174

				127.11		100.6174

				127.13		100.6174

				127.15		100.6174

				127.17		100.6174

				127.19		100.6174

				127.22		100.6174

				127.24		100.6174

				127.26		100.6174

				127.28		100.6174

				127.3		100.6174

				127.32		100.6174

				127.34		100.6174

				127.36		100.6174

				127.38		100.6174

				127.41		100.6174

				127.43		100.6174

				127.45		100.6174

				127.47		100.6174

				127.49		100.6174

				127.51		100.6174

				127.53		100.6174

				127.55		100.6174

				127.58		100.6174

				127.6		100.6174

				127.62		100.6174

				127.64		100.6174

				127.66		100.6174

				127.68		100.6174

				127.7		100.6174

				127.72		100.6174

				127.74		100.6174

				127.77		100.6174

				127.79		100.6174

				127.81		100.6174

				127.83		100.6174

				127.85		100.6174

				127.87		100.6174

				127.89		100.6174

				127.91		100.6174

				127.93		100.6134

				127.96		100.6134

				127.98		100.6134

				128		100.6134

				128.02		100.6134

				128.04		100.6134

				128.06		100.6134

				128.08		100.6134

				128.1		100.6134

				128.12		100.6134

				128.15		100.6134

				128.17		100.6134

				128.19		100.6134

				128.21		100.6134

				128.23		100.6134

				128.25		100.6134

				128.27		100.6134

				128.29		100.6134

				128.31		100.6134

				128.34		100.6134

				128.36		100.6134

				128.38		100.6134

				128.4		100.6134

				128.42		100.6134

				128.44		100.6134

				128.46		100.6093

				128.48		100.6134

				128.5		100.6134

				128.53		100.6134

				128.55		100.6134

				128.57		100.6093

				128.59		100.6093

				128.61		100.6093

				128.63		100.6093

				128.65		100.6093

				128.67		100.6093

				128.69		100.6093

				128.72		100.6093

				128.74		100.6093

				128.76		100.6093

				128.78		100.6093

				128.8		100.6093

				128.82		100.6093

				128.84		100.6093

				128.86		100.6093

				128.88		100.6093

				128.91		100.6093

				128.93		100.6093

				128.95		100.6093

				128.97		100.6093

				128.99		100.6093

				129.01		100.6093

				129.03		100.6093

				129.05		100.6093

				129.07		100.6093

				129.1		100.6052

				129.12		100.6052

				129.14		100.6052

				129.16		100.6052

				129.18		100.6052

				129.2		100.6052

				129.22		100.6052

				129.24		100.6052

				129.26		100.6052

				129.29		100.6052

				129.31		100.6052

				129.33		100.6052

				129.35		100.6052

				129.37		100.6012

				129.39		100.6052

				129.41		100.6012

				129.43		100.6012

				129.45		100.6012

				129.48		100.6012

				129.5		100.6012

				129.52		100.6012

				129.54		100.6012

				129.56		100.6012

				129.58		100.6012

				129.6		100.6012

				129.62		100.6012

				129.65		100.6012

				129.67		100.6012

				129.69		100.6012

				129.71		100.6012

				129.73		100.6012

				129.75		100.6012

				129.77		100.6012

				129.79		100.6012

				129.81		100.6012

				129.84		100.6012

				129.86		100.6012

				129.88		100.6012

				129.9		100.6012

				129.92		100.6012

				129.94		100.6012

				129.96		100.6012

				129.98		100.6012

				130		100.6012

				130.03		100.6012

				130.05		100.6012

				130.07		100.6012

				130.09		100.6012

				130.11		100.6012

				130.13		100.6012

				130.15		100.6012

				130.17		100.6012

				130.19		100.6052

				130.22		100.6012

				130.24		100.6012

				130.26		100.6012

				130.28		100.6012

				130.3		100.6012

				130.32		100.6012

				130.34		100.6012

				130.36		100.6012

				130.38		100.6012

				130.41		100.6012

				130.43		100.6012

				130.45		100.6012

				130.47		100.6012

				130.49		100.6012

				130.51		100.6012

				130.53		100.6012

				130.55		100.6012

				130.58		100.6012

				130.6		100.6012

				130.62		100.6012

				130.64		100.6012

				130.66		100.6012

				130.68		100.6012

				130.7		100.6012

				130.72		100.6012

				130.74		100.6012

				130.77		100.6012

				130.79		100.6012

				130.81		100.6012

				130.83		100.6012

				130.85		100.6012

				130.87		100.6012

				130.89		100.6012

				130.91		100.6012

				130.93		100.6012

				130.96		100.6012

				130.98		100.6012

				131		100.6012

				131.02		100.6012

				131.04		100.6012

				131.06		100.5971

				131.08		100.5971

				131.1		100.5971

				131.12		100.5971

				131.15		100.5971

				131.17		100.5971

				131.19		100.6012

				131.21		100.5971

				131.23		100.5971

				131.25		100.5971

				131.27		100.5971

				131.29		100.6012

				131.31		100.5971

				131.34		100.6012

				131.36		100.5971

				131.38		100.5971

				131.4		100.5971

				131.42		100.5971

				131.44		100.5971

				131.46		100.5971

				131.48		100.5971

				131.5		100.5971

				131.53		100.5971

				131.55		100.5971

				131.57		100.5971

				131.59		100.5971

				131.61		100.5971

				131.63		100.5971

				131.65		100.5971

				131.67		100.5971

				131.69		100.5971

				131.72		100.5971

				131.74		100.5971

				131.76		100.5971

				131.78		100.5971

				131.8		100.5971

				131.82		100.5971

				131.84		100.5971

				131.86		100.5971

				131.88		100.5971

				131.91		100.5971

				131.93		100.5971

				131.95		100.5971

				131.97		100.5971

				131.99		100.5971

				132.01		100.5971

				132.03		100.5971

				132.05		100.5931

				132.08		100.5971

				132.1		100.5931

				132.12		100.5931

				132.14		100.5931

				132.16		100.5931

				132.18		100.5931

				132.2		100.5931

				132.22		100.5931

				132.24		100.5931

				132.27		100.5931

				132.29		100.5931

				132.31		100.5931

				132.33		100.5931

				132.35		100.5931

				132.37		100.5931

				132.39		100.5931

				132.41		100.5931

				132.43		100.5931

				132.46		100.5931

				132.48		100.5931

				132.5		100.5931

				132.52		100.5931

				132.54		100.5931

				132.56		100.5931

				132.58		100.589

				132.6		100.589

				132.63		100.589

				132.65		100.589

				132.67		100.589

				132.69		100.589

				132.71		100.589

				132.73		100.589

				132.75		100.589

				132.77		100.589

				132.79		100.589

				132.82		100.589

				132.84		100.589

				132.86		100.589

				132.88		100.589

				132.9		100.5849

				132.92		100.5849

				132.94		100.5849

				132.96		100.5849

				132.98		100.5849

				133.01		100.5849

				133.03		100.5849

				133.05		100.5849

				133.07		100.5849

				133.09		100.5849

				133.11		100.5849

				133.13		100.5849

				133.15		100.5849

				133.17		100.5849

				133.2		100.5849

				133.22		100.5849

				133.24		100.5849

				133.26		100.5849

				133.28		100.5849

				133.3		100.5849

				133.32		100.5849

				133.34		100.5849

				133.37		100.5849

				133.39		100.5849

				133.41		100.5849

				133.43		100.5809

				133.45		100.5849

				133.47		100.5849

				133.49		100.5809

				133.51		100.5809

				133.53		100.5809

				133.56		100.5809

				133.58		100.5809

				133.6		100.5809

				133.62		100.5809

				133.64		100.5809

				133.66		100.5809

				133.68		100.5809

				133.7		100.5809

				133.72		100.5809

				133.75		100.5809

				133.77		100.5809

				133.79		100.5809

				133.81		100.5809

				133.83		100.5809

				133.85		100.5809

				133.87		100.5809

				133.89		100.5809

				133.92		100.5809

				133.94		100.5809

				133.96		100.5809

				133.98		100.5809

				134		100.5809

				134.02		100.5809

				134.04		100.5809

				134.06		100.5809

				134.08		100.5768

				134.11		100.5768

				134.13		100.5768

				134.15		100.5768

				134.17		100.5768

				134.19		100.5768

				134.21		100.5768

				134.23		100.5768

				134.25		100.5768

				134.27		100.5768

				134.3		100.5768

				134.32		100.5768

				134.34		100.5768

				134.36		100.5768

				134.38		100.5768

				134.4		100.5768

				134.42		100.5768

				134.44		100.5728

				134.47		100.5768

				134.49		100.5768

				134.51		100.5768

				134.53		100.5768

				134.55		100.5768

				134.57		100.5768

				134.59		100.5768

				134.61		100.5768

				134.63		100.5768

				134.66		100.5768

				134.68		100.5768

				134.7		100.5768

				134.72		100.5768

				134.74		100.5768

				134.76		100.5768

				134.78		100.5768

				134.8		100.5768

				134.82		100.5768

				134.85		100.5768

				134.87		100.5768

				134.89		100.5768

				134.91		100.5768

				134.93		100.5728

				134.95		100.5728

				134.97		100.5768

				134.99		100.5768

				135.01		100.5728

				135.04		100.5768

				135.06		100.5728

				135.08		100.5728

				135.1		100.5728

				135.12		100.5728

				135.14		100.5728

				135.16		100.5728

				135.18		100.5728

				135.21		100.5728

				135.23		100.5728

				135.25		100.5728

				135.27		100.5728

				135.29		100.5728

				135.31		100.5728

				135.33		100.5728

				135.35		100.5728

				135.37		100.5728

				135.4		100.5728

				135.42		100.5728

				135.44		100.5728

				135.46		100.5728

				135.48		100.5728

				135.5		100.5728

				135.52		100.5728

				135.54		100.5728

				135.56		100.5728

				135.59		100.5728

				135.61		100.5728

				135.63		100.5728

				135.65		100.5728

				135.67		100.5728

				135.69		100.5728

				135.71		100.5728

				135.73		100.5728

				135.76		100.5728

				135.78		100.5728

				135.8		100.5728

				135.82		100.5728

				135.84		100.5728

				135.86		100.5728

				135.88		100.5728

				135.9		100.5728

				135.92		100.5728

				135.95		100.5728

				135.97		100.5728

				135.99		100.5728

				136.01		100.5728

				136.03		100.5687

				136.05		100.5728

				136.07		100.5728

				136.09		100.5687

				136.11		100.5687

				136.14		100.5687

				136.16		100.5687

				136.18		100.5687

				136.2		100.5687

				136.22		100.5687

				136.24		100.5687

				136.26		100.5687

				136.28		100.5687

				136.31		100.5687

				136.33		100.5687

				136.35		100.5687

				136.37		100.5687

				136.39		100.5687

				136.41		100.5687

				136.43		100.5687

				136.45		100.5687

				136.47		100.5687

				136.5		100.5687

				136.52		100.5687

				136.54		100.5687

				136.56		100.5646

				136.58		100.5646

				136.6		100.5646

				136.62		100.5646

				136.64		100.5646

				136.67		100.5646

				136.69		100.5606

				136.71		100.5646

				136.73		100.5646

				136.75		100.5646

				136.77		100.5606

				136.79		100.5606

				136.81		100.5606

				136.83		100.5606

				136.86		100.5606

				136.88		100.5606

				136.9		100.5606

				136.92		100.5606

				136.94		100.5606

				136.96		100.5606

				136.98		100.5606

				137		100.5606

				137.03		100.5606

				137.05		100.5606

				137.07		100.5606

				137.09		100.5606

				137.11		100.5606

				137.13		100.5606

				137.15		100.5606

				137.17		100.5606

				137.19		100.5606

				137.22		100.5606

				137.24		100.5606

				137.26		100.5606

				137.28		100.5606

				137.3		100.5606

				137.32		100.5606

				137.34		100.5565

				137.36		100.5565

				137.39		100.5565

				137.41		100.5565

				137.43		100.5565

				137.45		100.5606

				137.47		100.5565

				137.49		100.5565

				137.51		100.5565

				137.53		100.5565

				137.55		100.5565

				137.58		100.5565

				137.6		100.5565

				137.62		100.5565

				137.64		100.5565

				137.66		100.5565

				137.68		100.5565

				137.7		100.5565

				137.72		100.5565

				137.75		100.5565

				137.77		100.5565

				137.79		100.5565

				137.81		100.5565

				137.83		100.5565

				137.85		100.5524

				137.87		100.5524

				137.89		100.5524

				137.91		100.5524

				137.94		100.5524

				137.96		100.5524

				137.98		100.5524

				138		100.5524

				138.02		100.5524

				138.04		100.5524

				138.06		100.5524

				138.08		100.5524

				138.1		100.5524

				138.13		100.5524

				138.15		100.5524

				138.17		100.5524

				138.19		100.5524

				138.21		100.5524

				138.23		100.5524

				138.25		100.5524

				138.27		100.5524

				138.3		100.5524

				138.32		100.5524

				138.34		100.5524

				138.36		100.5524

				138.38		100.5524

				138.4		100.5484

				138.42		100.5484

				138.44		100.5484

				138.46		100.5484

				138.49		100.5484

				138.51		100.5484

				138.53		100.5484

				138.55		100.5484

				138.57		100.5484

				138.59		100.5484

				138.61		100.5484

				138.63		100.5484

				138.66		100.5484

				138.68		100.5484

				138.7		100.5484

				138.72		100.5484

				138.74		100.5484

				138.76		100.5484

				138.78		100.5484

				138.8		100.5484

				138.83		100.5484

				138.85		100.5484

				138.87		100.5484

				138.89		100.5484

				138.91		100.5484

				138.93		100.5484

				138.95		100.5484

				138.97		100.5484

				138.99		100.5443

				139.02		100.5443

				139.04		100.5443

				139.06		100.5443

				139.08		100.5443

				139.1		100.5443

				139.12		100.5443

				139.14		100.5443

				139.16		100.5443

				139.19		100.5443

				139.21		100.5443

				139.23		100.5443

				139.25		100.5443

				139.27		100.5443

				139.29		100.5443

				139.31		100.5443

				139.33		100.5403

				139.35		100.5403

				139.38		100.5403

				139.4		100.5403

				139.42		100.5403

				139.44		100.5403

				139.46		100.5403

				139.48		100.5403

				139.5		100.5403

				139.52		100.5403

				139.55		100.5403

				139.57		100.5403

				139.59		100.5403

				139.61		100.5403

				139.63		100.5403

				139.65		100.5403

				139.67		100.5362

				139.69		100.5362

				139.72		100.5362

				139.74		100.5362

				139.76		100.5362

				139.78		100.5362

				139.8		100.5362

				139.82		100.5362

				139.84		100.5321

				139.86		100.5321

				139.88		100.5321

				139.91		100.5321

				139.93		100.5321

				139.95		100.5321

				139.97		100.5321

				139.99		100.5321

				140.01		100.5321

				140.03		100.5321

				140.05		100.5321

				140.08		100.5321

				140.1		100.5321

				140.12		100.5321

				140.14		100.5281

				140.16		100.5281

				140.18		100.5281

				140.2		100.5281

				140.22		100.5281

				140.24		100.5281

				140.27		100.524

				140.29		100.524

				140.31		100.524

				140.33		100.524

				140.35		100.524

				140.37		100.524

				140.39		100.524

				140.41		100.524

				140.44		100.524

				140.46		100.524

				140.48		100.5199

				140.5		100.5199

				140.52		100.5199

				140.54		100.5199

				140.56		100.5199

				140.58		100.5199

				140.6		100.5199

				140.63		100.5199

				140.65		100.5199

				140.67		100.5159

				140.69		100.5159

				140.71		100.5159

				140.73		100.5159

				140.75		100.5159

				140.77		100.5159

				140.8		100.5159

				140.82		100.5159

				140.84		100.5159

				140.86		100.5118

				140.88		100.5118

				140.9		100.5118

				140.92		100.5118

				140.94		100.5118

				140.97		100.5118

				140.99		100.5118

				141.01		100.5118

				141.03		100.5118

				141.05		100.5118

				141.07		100.5118

				141.09		100.5118

				141.11		100.5118

				141.13		100.5118

				141.16		100.5118

				141.18		100.5078

				141.2		100.5078

				141.22		100.5078

				141.24		100.5078

				141.26		100.5078

				141.28		100.5078

				141.3		100.5078

				141.33		100.5078

				141.35		100.5078

				141.37		100.5078

				141.39		100.5078

				141.41		100.5078

				141.43		100.5078

				141.45		100.5078

				141.47		100.5037

				141.5		100.5037

				141.52		100.5037

				141.54		100.5037

				141.56		100.5037

				141.58		100.5037

				141.6		100.5037

				141.62		100.5037

				141.64		100.5037

				141.66		100.5037

				141.69		100.5037

				141.71		100.5037

				141.73		100.5037

				141.75		100.4996

				141.77		100.4996

				141.79		100.4996

				141.81		100.4996

				141.83		100.4996

				141.86		100.4996

				141.88		100.4996

				141.9		100.4996

				141.92		100.4996

				141.94		100.4996

				141.96		100.4996

				141.98		100.4996

				142		100.4996

				142.03		100.4956

				142.05		100.4956

				142.07		100.4956

				142.09		100.4956

				142.11		100.4956

				142.13		100.4956

				142.15		100.4956

				142.17		100.4956

				142.19		100.4956

				142.22		100.4956

				142.24		100.4956

				142.26		100.4915

				142.28		100.4915

				142.3		100.4956

				142.32		100.4915

				142.34		100.4915

				142.36		100.4915

				142.39		100.4915

				142.41		100.4915

				142.43		100.4915

				142.45		100.4915

				142.47		100.4915

				142.49		100.4915

				142.51		100.4915

				142.53		100.4915

				142.56		100.4915

				142.58		100.4915

				142.6		100.4915

				142.62		100.4915

				142.64		100.4915

				142.66		100.4915

				142.68		100.4915

				142.7		100.4915

				142.72		100.4874

				142.75		100.4874

				142.77		100.4874

				142.79		100.4874

				142.81		100.4874

				142.83		100.4874

				142.85		100.4874

				142.87		100.4874

				142.89		100.4874

				142.92		100.4874

				142.94		100.4874

				142.96		100.4874

				142.98		100.4874

				143		100.4874

				143.02		100.4834

				143.04		100.4834

				143.06		100.4834

				143.09		100.4834

				143.11		100.4834

				143.13		100.4834

				143.15		100.4834

				143.17		100.4834

				143.19		100.4834

				143.21		100.4834

				143.23		100.4834

				143.26		100.4793

				143.28		100.4793

				143.3		100.4793

				143.32		100.4793

				143.34		100.4793

				143.36		100.4793

				143.38		100.4793

				143.4		100.4793

				143.42		100.4793

				143.45		100.4793

				143.47		100.4793

				143.49		100.4793

				143.51		100.4753

				143.53		100.4753

				143.55		100.4753

				143.57		100.4753

				143.59		100.4753

				143.62		100.4753

				143.64		100.4753

				143.66		100.4753

				143.68		100.4753

				143.7		100.4753

				143.72		100.4712

				143.74		100.4712

				143.76		100.4712

				143.79		100.4712

				143.81		100.4712

				143.83		100.4712

				143.85		100.4712

				143.87		100.4712

				143.89		100.4712

				143.91		100.4712

				143.93		100.4712

				143.96		100.4712

				143.98		100.4671

				144		100.4671

				144.02		100.4671

				144.04		100.4671

				144.06		100.4671

				144.08		100.4671

				144.1		100.4671

				144.13		100.4671

				144.15		100.4671

				144.17		100.4671

				144.19		100.4631

				144.21		100.4631

				144.23		100.4631

				144.25		100.4631

				144.27		100.4631

				144.3		100.4631

				144.32		100.4631

				144.34		100.4631

				144.36		100.4631

				144.38		100.4631

				144.4		100.4631

				144.42		100.4631

				144.44		100.4631

				144.47		100.4631

				144.49		100.459

				144.51		100.459

				144.53		100.459

				144.55		100.459

				144.57		100.459

				144.59		100.459

				144.61		100.459

				144.64		100.455

				144.66		100.455

				144.68		100.455

				144.7		100.455

				144.72		100.455

				144.74		100.455

				144.76		100.455

				144.78		100.4509

				144.81		100.4509

				144.83		100.4509

				144.85		100.4509

				144.87		100.4509

				144.89		100.4509

				144.91		100.4509

				144.93		100.4509

				144.95		100.4509

				144.98		100.4509

				145		100.4468

				145.02		100.4468

				145.04		100.4468

				145.06		100.4468

				145.08		100.4468

				145.1		100.4468

				145.12		100.4468

				145.14		100.4428

				145.17		100.4428

				145.19		100.4428

				145.21		100.4428

				145.23		100.4428

				145.25		100.4428

				145.27		100.4428

				145.29		100.4428

				145.31		100.4387

				145.34		100.4387

				145.36		100.4387

				145.38		100.4387

				145.4		100.4346

				145.42		100.4346

				145.44		100.4346

				145.46		100.4346

				145.48		100.4346

				145.51		100.4346

				145.53		100.4306

				145.55		100.4306

				145.57		100.4306

				145.59		100.4306

				145.61		100.4306

				145.63		100.4306

				145.65		100.4306

				145.68		100.4265

				145.7		100.4265

				145.72		100.4265

				145.74		100.4265

				145.76		100.4265

				145.78		100.4265

				145.8		100.4265

				145.82		100.4265

				145.85		100.4265

				145.87		100.4265

				145.89		100.4265

				145.91		100.4265

				145.93		100.4225

				145.95		100.4225

				145.97		100.4225

				145.99		100.4225

				146.02		100.4225

				146.04		100.4225

				146.06		100.4225

				146.08		100.4184

				146.1		100.4184

				146.12		100.4184

				146.14		100.4184

				146.16		100.4184

				146.19		100.4184

				146.21		100.4184

				146.23		100.4143

				146.25		100.4143

				146.27		100.4143

				146.29		100.4143

				146.31		100.4143

				146.33		100.4143

				146.36		100.4103

				146.38		100.4103

				146.4		100.4103

				146.42		100.4103

				146.44		100.4103

				146.46		100.4103

				146.48		100.4062

				146.5		100.4062

				146.53		100.4062

				146.55		100.4062

				146.57		100.4062

				146.59		100.4062

				146.61		100.4062

				146.63		100.4021

				146.65		100.4021

				146.67		100.4021

				146.7		100.4021

				146.72		100.4021

				146.74		100.4021

				146.76		100.4021

				146.78		100.4021

				146.8		100.4021

				146.82		100.4021

				146.84		100.4021

				146.87		100.4021

				146.89		100.4021

				146.91		100.4021

				146.93		100.4021

				146.95		100.4021

				146.97		100.4021

				146.99		100.4021

				147.01		100.4021

				147.04		100.4021

				147.06		100.3981

				147.08		100.3981

				147.1		100.3981

				147.12		100.3981

				147.14		100.3981

				147.16		100.3981

				147.18		100.3981

				147.21		100.3981

				147.23		100.3981

				147.25		100.3981

				147.27		100.3981

				147.29		100.3981

				147.31		100.3981

				147.33		100.3981

				147.35		100.3981

				147.38		100.3981

				147.4		100.3981

				147.42		100.3981

				147.44		100.394

				147.46		100.394

				147.48		100.394

				147.5		100.394

				147.52		100.394

				147.55		100.394

				147.57		100.394

				147.59		100.394

				147.61		100.394

				147.63		100.394

				147.65		100.394

				147.67		100.39

				147.69		100.39

				147.72		100.39

				147.74		100.39

				147.76		100.39

				147.78		100.39

				147.8		100.39

				147.82		100.39

				147.84		100.39

				147.86		100.3859

				147.89		100.3859

				147.91		100.3859

				147.93		100.3859

				147.95		100.3859

				147.97		100.3859

				147.99		100.3859

				148.01		100.3859

				148.03		100.3859

				148.06		100.3859

				148.08		100.3859

				148.1		100.3859

				148.12		100.3859

				148.14		100.3859

				148.16		100.3818

				148.18		100.3818

				148.2		100.3818

				148.23		100.3818

				148.25		100.3818

				148.27		100.3818

				148.29		100.3818

				148.31		100.3818

				148.33		100.3818

				148.35		100.3818

				148.37		100.3818

				148.4		100.3778

				148.42		100.3778

				148.44		100.3778

				148.46		100.3778

				148.48		100.3778

				148.5		100.3778

				148.52		100.3778

				148.54		100.3778

				148.57		100.3778

				148.59		100.3778

				148.61		100.3778

				148.63		100.3778

				148.65		100.3778

				148.67		100.3778

				148.69		100.3778

				148.71		100.3737

				148.73		100.3737

				148.76		100.3737

				148.78		100.3737

				148.8		100.3737

				148.82		100.3737

				148.84		100.3696

				148.86		100.3696

				148.88		100.3696

				148.9		100.3696

				148.93		100.3696

				148.95		100.3696

				148.97		100.3656

				148.99		100.3656

				149.01		100.3656

				149.03		100.3656

				149.05		100.3615

				149.07		100.3615

				149.1		100.3615

				149.12		100.3615

				149.14		100.3615

				149.16		100.3615

				149.18		100.3575

				149.2		100.3575

				149.22		100.3575

				149.24		100.3575

				149.27		100.3575

				149.29		100.3575

				149.31		100.3534

				149.33		100.3534

				149.35		100.3534

				149.37		100.3534

				149.39		100.3534

				149.41		100.3534

				149.44		100.3493

				149.46		100.3493

				149.48		100.3493

				149.5		100.3493

				149.52		100.3493

				149.54		100.3493

				149.56		100.3453

				149.58		100.3453

				149.61		100.3453

				149.63		100.3453

				149.65		100.3453

				149.67		100.3453

				149.69		100.3453

				149.71		100.3453

				149.73		100.3453

				149.75		100.3453

				149.78		100.3412

				149.8		100.3412

				149.82		100.3412

				149.84		100.3412

				149.86		100.3412

				149.88		100.3412

				149.9		100.3412

				149.92		100.3372

				149.95		100.3372

				149.97		100.3372

				149.99		100.3372

				150.01		100.3372

				150.03		100.3372

				150.05		100.3372

				150.07		100.3372

				150.09		100.3331

				150.12		100.3331

				150.14		100.3331

				150.16		100.3331

				150.18		100.3331

				150.2		100.3331

				150.22		100.329

				150.24		100.329

				150.26		100.329

				150.29		100.329

				150.31		100.329

				150.33		100.329

				150.35		100.325

				150.37		100.325

				150.39		100.325

				150.41		100.325

				150.43		100.325

				150.46		100.325

				150.48		100.325

				150.5		100.3209

				150.52		100.3209

				150.54		100.3209

				150.56		100.3209

				150.58		100.3209

				150.6		100.3209

				150.62		100.3209

				150.65		100.3209

				150.67		100.3168

				150.69		100.3209

				150.71		100.3168

				150.73		100.3168

				150.75		100.3168

				150.77		100.3168

				150.79		100.3168

				150.82		100.3168

				150.84		100.3128

				150.86		100.3128

				150.88		100.3128

				150.9		100.3128

				150.92		100.3128

				150.94		100.3128

				150.96		100.3128

				150.99		100.3128

				151.01		100.3087

				151.03		100.3087

				151.05		100.3087

				151.07		100.3087

				151.09		100.3087

				151.11		100.3087

				151.13		100.3087

				151.15		100.3047

				151.18		100.3047

				151.2		100.3047

				151.22		100.3047

				151.24		100.3047

				151.26		100.3006

				151.28		100.3006

				151.3		100.3006

				151.32		100.3006

				151.35		100.3006

				151.37		100.2965

				151.39		100.2965

				151.41		100.2965

				151.43		100.2965

				151.45		100.2965

				151.47		100.2965

				151.49		100.2965

				151.52		100.2965

				151.54		100.2925

				151.56		100.2925

				151.58		100.2925

				151.6		100.2925

				151.62		100.2925

				151.64		100.2884

				151.66		100.2884

				151.69		100.2884

				151.71		100.2884

				151.73		100.2884

				151.75		100.2843

				151.77		100.2843

				151.79		100.2843

				151.81		100.2843

				151.83		100.2843

				151.85		100.2843

				151.88		100.2843

				151.9		100.2803

				151.92		100.2803

				151.94		100.2803

				151.96		100.2762

				151.98		100.2762

				152		100.2762

				152.02		100.2762

				152.05		100.2762

				152.07		100.2762

				152.09		100.2762

				152.11		100.2722

				152.13		100.2722

				152.15		100.2722

				152.17		100.2722

				152.19		100.2681

				152.22		100.2681

				152.24		100.2681

				152.26		100.2681

				152.28		100.264

				152.3		100.264

				152.32		100.264

				152.34		100.264

				152.36		100.264

				152.39		100.26

				152.41		100.26

				152.43		100.26

				152.45		100.26

				152.47		100.2559

				152.49		100.2559

				152.51		100.2559

				152.53		100.2559

				152.56		100.2518

				152.58		100.2518

				152.6		100.2518

				152.62		100.2518

				152.64		100.2518

				152.66		100.2518

				152.68		100.2518

				152.7		100.2478

				152.72		100.2478

				152.75		100.2478

				152.77		100.2478

				152.79		100.2478

				152.81		100.2478

				152.83		100.2437

				152.85		100.2437

				152.87		100.2437

				152.89		100.2437

				152.92		100.2397

				152.94		100.2397

				152.96		100.2397

				152.98		100.2397

				153		100.2397

				153.02		100.2397

				153.04		100.2356

				153.06		100.2356

				153.09		100.2356

				153.11		100.2356

				153.13		100.2356

				153.15		100.2315

				153.17		100.2315

				153.19		100.2315

				153.21		100.2315

				153.23		100.2315

				153.26		100.2315

				153.28		100.2315

				153.3		100.2275

				153.32		100.2275

				153.34		100.2275

				153.36		100.2275

				153.38		100.2275

				153.4		100.2275

				153.43		100.2234

				153.45		100.2234

				153.47		100.2234

				153.49		100.2234

				153.51		100.2234

				153.53		100.2234

				153.55		100.2194

				153.57		100.2194

				153.6		100.2194

				153.62		100.2194

				153.64		100.2194

				153.66		100.2194

				153.68		100.2194

				153.7		100.2194

				153.72		100.2194

				153.74		100.2153

				153.77		100.2153

				153.79		100.2153

				153.81		100.2153

				153.83		100.2153

				153.85		100.2153

				153.87		100.2112

				153.89		100.2112

				153.91		100.2112

				153.93		100.2112

				153.96		100.2112

				153.98		100.2112

				154		100.2072

				154.02		100.2072

				154.04		100.2072

				154.06		100.2072

				154.08		100.2072

				154.1		100.2031

				154.13		100.2031

				154.15		100.2031

				154.17		100.2031

				154.19		100.2031

				154.21		100.199

				154.23		100.199

				154.25		100.199

				154.27		100.199

				154.3		100.199

				154.32		100.195

				154.34		100.195

				154.36		100.195

				154.38		100.195

				154.4		100.195

				154.42		100.1909

				154.44		100.195

				154.46		100.1909

				154.49		100.1909

				154.51		100.1909

				154.53		100.1909

				154.55		100.1909

				154.57		100.1909

				154.59		100.1869

				154.61		100.1869

				154.63		100.1869

				154.66		100.1869

				154.68		100.1869

				154.7		100.1828

				154.72		100.1828

				154.74		100.1828

				154.76		100.1828

				154.78		100.1828

				154.8		100.1828

				154.83		100.1828

				154.85		100.1787

				154.87		100.1787

				154.89		100.1787

				154.91		100.1787

				154.93		100.1747

				154.95		100.1747

				154.97		100.1747

				154.99		100.1747

				155.02		100.1747

				155.04		100.1747

				155.06		100.1706

				155.08		100.1706

				155.1		100.1706

				155.12		100.1706

				155.14		100.1706

				155.16		100.1665

				155.19		100.1665

				155.21		100.1665

				155.23		100.1665

				155.25		100.1665

				155.27		100.1665

				155.29		100.1625

				155.31		100.1625

				155.33		100.1625

				155.35		100.1625

				155.38		100.1625

				155.4		100.1625

				155.42		100.1584

				155.44		100.1584

				155.46		100.1584

				155.48		100.1584

				155.5		100.1584

				155.52		100.1544

				155.54		100.1544

				155.57		100.1544

				155.59		100.1544

				155.61		100.1544

				155.63		100.1544

				155.65		100.1544

				155.67		100.1503

				155.69		100.1503

				155.71		100.1503

				155.74		100.1503

				155.76		100.1462

				155.78		100.1462

				155.8		100.1462

				155.82		100.1462

				155.84		100.1462

				155.86		100.1422

				155.88		100.1422

				155.9		100.1422

				155.93		100.1422

				155.95		100.1381

				155.97		100.1381

				155.99		100.1381

				156.01		100.134

				156.03		100.134

				156.05		100.134

				156.07		100.134

				156.1		100.134

				156.12		100.13

				156.14		100.134

				156.16		100.13

				156.18		100.13

				156.2		100.13

				156.22		100.1259

				156.24		100.1259

				156.26		100.1259

				156.29		100.1259

				156.31		100.1259

				156.33		100.1259

				156.35		100.1219

				156.37		100.1219

				156.39		100.1219

				156.41		100.1178

				156.43		100.1178

				156.45		100.1178

				156.48		100.1178

				156.5		100.1137

				156.52		100.1137

				156.54		100.1137

				156.56		100.1137

				156.58		100.1097

				156.6		100.1097

				156.62		100.1097

				156.65		100.1097

				156.67		100.1097

				156.69		100.1097

				156.71		100.1056

				156.73		100.1056

				156.75		100.1056

				156.77		100.1056

				156.79		100.1056

				156.81		100.1016

				156.84		100.1016

				156.86		100.1016

				156.88		100.1016

				156.9		100.1016

				156.92		100.0975

				156.94		100.0975

				156.96		100.0975

				156.98		100.0975

				157.01		100.0934

				157.03		100.0934

				157.05		100.0934

				157.07		100.0934

				157.09		100.0934

				157.11		100.0934

				157.13		100.0894

				157.15		100.0894

				157.17		100.0894

				157.2		100.0894

				157.22		100.0853

				157.24		100.0853

				157.26		100.0853

				157.28		100.0853

				157.3		100.0812

				157.32		100.0812

				157.34		100.0812

				157.37		100.0812

				157.39		100.0772

				157.41		100.0772

				157.43		100.0772

				157.45		100.0772

				157.47		100.0731

				157.49		100.0731

				157.51		100.0731

				157.53		100.0731

				157.56		100.0731

				157.58		100.0691

				157.6		100.0691

				157.62		100.0691

				157.64		100.0691

				157.66		100.0691

				157.68		100.0691

				157.7		100.065

				157.73		100.065

				157.75		100.065

				157.77		100.065

				157.79		100.0609

				157.81		100.0609

				157.83		100.0609

				157.85		100.0569

				157.87		100.0569

				157.89		100.0569

				157.92		100.0528

				157.94		100.0528

				157.96		100.0528

				157.98		100.0528

				158		100.0528

				158.02		100.0487

				158.04		100.0487

				158.06		100.0487

				158.08		100.0487

				158.11		100.0487

				158.13		100.0447

				158.15		100.0447

				158.17		100.0447

				158.19		100.0447

				158.21		100.0406

				158.23		100.0406

				158.25		100.0406

				158.27		100.0406

				158.3		100.0366

				158.32		100.0366

				158.34		100.0366

				158.36		100.0366

				158.38		100.0325

				158.4		100.0325

				158.42		100.0325

				158.44		100.0325

				158.47		100.0325

				158.49		100.0284

				158.51		100.0284

				158.53		100.0284

				158.55		100.0284

				158.57		100.0244

				158.59		100.0244

				158.61		100.0203

				158.63		100.0203

				158.66		100.0203

				158.68		100.0162

				158.7		100.0162

				158.72		100.0162

				158.74		100.0122

				158.76		100.0122

				158.78		100.0122

				158.8		100.0081

				158.82		100.0081

				158.85		100.0081

				158.87		100.0081

				158.89		100.0081

				158.91		100.0041

				158.93		100.0041

				158.95		100.0041

				158.97		100

				158.99		100

				159.01		100

				159.04		100

				159.06		100

				159.08		99.99594

				159.1		99.99594

				159.12		99.99594

				159.14		99.99188

				159.16		99.99188

				159.18		99.99188

				159.2		99.99188

				159.23		99.98781

				159.25		99.98781

				159.27		99.98781

				159.29		99.98781

				159.31		99.98375

				159.33		99.98375

				159.35		99.97969

				159.37		99.97969

				159.4		99.97969

				159.42		99.97563

				159.44		99.97563

				159.46		99.97563

				159.48		99.97563

				159.5		99.97157

				159.52		99.97157

				159.54		99.97157

				159.56		99.97157

				159.59		99.97157

				159.61		99.97157

				159.63		99.97157

				159.65		99.9675

				159.67		99.9675

				159.69		99.9675

				159.71		99.9675

				159.73		99.96344

				159.75		99.96344

				159.78		99.96344

				159.8		99.96344

				159.82		99.95938

				159.84		99.95938

				159.86		99.95938

				159.88		99.95532

				159.9		99.95532

				159.92		99.95532

				159.94		99.95126

				159.97		99.95126

				159.99		99.95126

				160.01		99.95126

				160.03		99.94719

				160.05		99.94719

				160.07		99.94719

				160.09		99.94719

				160.11		99.94719

				160.13		99.94313

				160.16		99.94313

				160.18		99.94313

				160.2		99.93907

				160.22		99.94313

				160.24		99.93907

				160.26		99.93907

				160.28		99.93907

				160.3		99.93907

				160.32		99.93501

				160.35		99.93501

				160.37		99.93501

				160.39		99.93501

				160.41		99.93501

				160.43		99.93094

				160.45		99.93094

				160.47		99.93094

				160.49		99.92688

				160.52		99.92688

				160.54		99.92688

				160.56		99.92688

				160.58		99.92282

				160.6		99.92282

				160.62		99.92282

				160.64		99.91876

				160.66		99.91876

				160.68		99.91876

				160.71		99.9147

				160.73		99.9147

				160.75		99.9147

				160.77		99.91063

				160.79		99.91063

				160.81		99.91063

				160.83		99.90657

				160.85		99.90657

				160.87		99.90657

				160.9		99.90657

				160.92		99.90251

				160.94		99.90251

				160.96		99.90251

				160.98		99.90251

				161		99.89845

				161.02		99.89845

				161.04		99.89845

				161.06		99.89845

				161.09		99.89439

				161.11		99.89439

				161.13		99.89439

				161.15		99.89032

				161.17		99.89032

				161.19		99.89032

				161.21		99.88626

				161.23		99.88626

				161.25		99.8822

				161.27		99.8822

				161.3		99.87814

				161.32		99.87814

				161.34		99.87814

				161.36		99.87408

				161.38		99.87408

				161.4		99.87001

				161.42		99.87001

				161.44		99.87001

				161.46		99.87001

				161.49		99.87001

				161.51		99.87001

				161.53		99.86595

				161.55		99.86595

				161.57		99.86595

				161.59		99.86595

				161.61		99.86189

				161.63		99.86189

				161.65		99.85783

				161.68		99.85783

				161.7		99.85783

				161.72		99.85377

				161.74		99.85377

				161.76		99.8497

				161.78		99.8497

				161.8		99.8497

				161.82		99.84564

				161.84		99.84158

				161.87		99.84158

				161.89		99.83752

				161.91		99.83752

				161.93		99.83346

				161.95		99.83346

				161.97		99.83346

				161.99		99.83346

				162.01		99.83346

				162.03		99.82939

				162.06		99.82939

				162.08		99.82939

				162.1		99.82939

				162.12		99.82533

				162.14		99.82533

				162.16		99.82127

				162.18		99.82127

				162.2		99.82127

				162.22		99.82127

				162.25		99.81721

				162.27		99.81721

				162.29		99.81721

				162.31		99.81314

				162.33		99.81314

				162.35		99.80908

				162.37		99.81314

				162.39		99.80908

				162.41		99.80908

				162.44		99.80908

				162.46		99.80502

				162.48		99.80502

				162.5		99.80502

				162.52		99.80502

				162.54		99.80502

				162.56		99.80502

				162.58		99.80096

				162.6		99.80096

				162.63		99.80096

				162.65		99.80096

				162.67		99.7969

				162.69		99.79283

				162.71		99.79283

				162.73		99.79283

				162.75		99.78877

				162.77		99.78877

				162.79		99.78471

				162.82		99.78471

				162.84		99.78065

				162.86		99.78065

				162.88		99.78065

				162.9		99.77659

				162.92		99.77659

				162.94		99.77252

				162.96		99.77252

				162.98		99.77252

				163.01		99.77252

				163.03		99.76846

				163.05		99.76846

				163.07		99.7644

				163.09		99.7644

				163.11		99.76034

				163.13		99.76034

				163.15		99.76034

				163.17		99.75628

				163.2		99.75628

				163.22		99.75628

				163.24		99.75221

				163.26		99.75221

				163.28		99.74815

				163.3		99.74815

				163.32		99.74409

				163.34		99.74409

				163.36		99.74409

				163.38		99.74409

				163.41		99.74003

				163.43		99.74003

				163.45		99.73597

				163.47		99.73597

				163.49		99.7319

				163.51		99.7319

				163.53		99.72784

				163.55		99.72784

				163.57		99.72784

				163.6		99.72784

				163.62		99.72378

				163.64		99.71972

				163.66		99.71972

				163.68		99.71972

				163.7		99.71566

				163.72		99.71566

				163.74		99.71566

				163.76		99.71566

				163.79		99.71159

				163.81		99.71159

				163.83		99.70753

				163.85		99.70753

				163.87		99.70753

				163.89		99.70753

				163.91		99.70753

				163.93		99.70347

				163.95		99.70347

				163.98		99.70347

				164		99.70347

				164.02		99.69941

				164.04		99.69941

				164.06		99.69941

				164.08		99.69534

				164.1		99.69534

				164.12		99.69534

				164.14		99.69534

				164.16		99.69534

				164.19		99.69128

				164.21		99.69128

				164.23		99.68722

				164.25		99.68722

				164.27		99.68722

				164.29		99.68316

				164.31		99.68316

				164.33		99.6791

				164.35		99.6791

				164.38		99.67503

				164.4		99.67503

				164.42		99.67503

				164.44		99.67097

				164.46		99.67097

				164.48		99.66691

				164.5		99.66285

				164.52		99.66285

				164.54		99.66285

				164.57		99.65879

				164.59		99.65879

				164.61		99.65472

				164.63		99.65472

				164.65		99.65066

				164.67		99.65066

				164.69		99.6466

				164.71		99.6466

				164.73		99.6466

				164.76		99.6466

				164.78		99.64254

				164.8		99.64254

				164.82		99.63848

				164.84		99.63848

				164.86		99.63848

				164.88		99.63441

				164.9		99.63441

				164.92		99.63441

				164.94		99.63035

				164.97		99.63035

				164.99		99.63035

				165.01		99.62629

				165.03		99.62629

				165.05		99.62223

				165.07		99.62223

				165.09		99.62223

				165.11		99.61817

				165.13		99.6141

				165.16		99.6141

				165.18		99.61004

				165.2		99.6141

				165.22		99.61004

				165.24		99.61004

				165.26		99.60598

				165.28		99.60598

				165.3		99.60598

				165.32		99.60598

				165.35		99.60192

				165.37		99.59786

				165.39		99.60192

				165.41		99.59786

				165.43		99.59786

				165.45		99.59379

				165.47		99.59379

				165.49		99.59379

				165.51		99.58973

				165.53		99.58973

				165.56		99.58973

				165.58		99.58567

				165.6		99.58567

				165.62		99.58567

				165.64		99.58161

				165.66		99.58161

				165.68		99.57754

				165.7		99.57754

				165.72		99.57754

				165.75		99.57754

				165.77		99.57754

				165.79		99.56942

				165.81		99.56942

				165.83		99.56942

				165.85		99.56536

				165.87		99.5613

				165.89		99.5613

				165.91		99.5613

				165.94		99.55723

				165.96		99.55723

				165.98		99.55317

				166		99.55317

				166.02		99.54911

				166.04		99.54505

				166.06		99.54505

				166.08		99.54505

				166.1		99.54505

				166.13		99.54099

				166.15		99.54099

				166.17		99.53692

				166.19		99.53286

				166.21		99.53286

				166.23		99.5288

				166.25		99.5288

				166.27		99.5288

				166.29		99.52474

				166.31		99.52474

				166.34		99.52474

				166.36		99.52068

				166.38		99.52068

				166.4		99.52068

				166.42		99.51661

				166.44		99.51661

				166.46		99.51255

				166.48		99.51255

				166.5		99.51255

				166.53		99.50849

				166.55		99.50849

				166.57		99.50443

				166.59		99.50443

				166.61		99.50037

				166.63		99.50037

				166.65		99.4963

				166.67		99.4963

				166.69		99.49224

				166.71		99.49224

				166.74		99.48818

				166.76		99.48818

				166.78		99.48818

				166.8		99.48412

				166.82		99.48412

				166.84		99.48412

				166.86		99.48412

				166.88		99.48006

				166.9		99.47599

				166.93		99.47599

				166.95		99.47193

				166.97		99.47193

				166.99		99.47193

				167.01		99.47193

				167.03		99.46787

				167.05		99.46787

				167.07		99.46381

				167.09		99.46381

				167.12		99.45974

				167.14		99.45974

				167.16		99.45974

				167.18		99.45568

				167.2		99.45568

				167.22		99.45162

				167.24		99.44756

				167.26		99.44756

				167.28		99.44756

				167.3		99.4435

				167.33		99.4435

				167.35		99.4435

				167.37		99.43943

				167.39		99.43943

				167.41		99.43537

				167.43		99.43131

				167.45		99.43131

				167.47		99.43131

				167.49		99.42725

				167.52		99.42725

				167.54		99.42725

				167.56		99.42319

				167.58		99.42319

				167.6		99.41912

				167.62		99.41912

				167.64		99.41506

				167.66		99.41506

				167.68		99.41506

				167.71		99.411

				167.73		99.411

				167.75		99.411

				167.77		99.40694

				167.79		99.40694

				167.81		99.40288

				167.83		99.40288

				167.85		99.40288

				167.87		99.40288

				167.89		99.39881

				167.92		99.39881

				167.94		99.39475

				167.96		99.39475

				167.98		99.39069

				168		99.39069

				168.02		99.38663

				168.04		99.38663

				168.06		99.38663

				168.08		99.38257

				168.11		99.38257

				168.13		99.3785

				168.15		99.3785

				168.17		99.3785

				168.19		99.37444

				168.21		99.37444

				168.23		99.37038

				168.25		99.37038

				168.27		99.36632

				168.29		99.36632

				168.32		99.36226

				168.34		99.36226

				168.36		99.36226

				168.38		99.35819

				168.4		99.35819

				168.42		99.35413

				168.44		99.35413

				168.46		99.35413

				168.48		99.35413

				168.51		99.35007

				168.53		99.35007

				168.55		99.35007

				168.57		99.34601

				168.59		99.34601

				168.61		99.34194

				168.63		99.34194

				168.65		99.33788

				168.67		99.33788

				168.69		99.33382

				168.72		99.32976

				168.74		99.32976

				168.76		99.32976

				168.78		99.3257

				168.8		99.3257

				168.82		99.32163

				168.84		99.32163

				168.86		99.31351

				168.88		99.30945

				168.91		99.30945

				168.93		99.30539

				168.95		99.30132

				168.97		99.30132

				168.99		99.29726

				169.01		99.29726

				169.03		99.2932

				169.05		99.2932

				169.07		99.28914

				169.09		99.28508

				169.12		99.28508

				169.14		99.28101

				169.16		99.27695

				169.18		99.27695

				169.2		99.27289

				169.22		99.27289

				169.24		99.27289

				169.26		99.27289

				169.28		99.26883

				169.3		99.26883

				169.33		99.26883

				169.35		99.26883

				169.37		99.26477

				169.39		99.26477

				169.41		99.26477

				169.43		99.26477

				169.45		99.2607

				169.47		99.2607

				169.49		99.25664

				169.52		99.25664

				169.54		99.24852

				169.56		99.24852

				169.58		99.24852

				169.6		99.24852

				169.62		99.24852

				169.64		99.24446

				169.66		99.24039

				169.68		99.23633

				169.7		99.23633

				169.73		99.22821

				169.75		99.22821

				169.77		99.22414

				169.79		99.22008

				169.81		99.22008

				169.83		99.21602

				169.85		99.21602

				169.87		99.21196

				169.89		99.2079

				169.92		99.2079

				169.94		99.19977

				169.96		99.19977

				169.98		99.19977

				170		99.19977

				170.02		99.19571

				170.04		99.19165

				170.06		99.18759

				170.08		99.18759

				170.1		99.18759

				170.13		99.18352

				170.15		99.17946

				170.17		99.17946

				170.19		99.17946

				170.21		99.1754

				170.23		99.1754

				170.25		99.17134

				170.27		99.16728

				170.29		99.16728

				170.31		99.16728

				170.34		99.16728

				170.36		99.16321

				170.38		99.16321

				170.4		99.15915

				170.42		99.15915

				170.44		99.15509

				170.46		99.15509

				170.48		99.15103

				170.5		99.15103

				170.53		99.14697

				170.55		99.1429

				170.57		99.13884

				170.59		99.13884

				170.61		99.13478

				170.63		99.13478

				170.65		99.12666

				170.67		99.12666

				170.69		99.12666

				170.71		99.12666

				170.74		99.12259

				170.76		99.11447

				170.78		99.11447

				170.8		99.11041

				170.82		99.11041

				170.84		99.10634

				170.86		99.10634

				170.88		99.10228

				170.9		99.10228

				170.92		99.09822

				170.95		99.09822

				170.97		99.09416

				170.99		99.09416

				171.01		99.0901

				171.03		99.08603

				171.05		99.08603

				171.07		99.08197

				171.09		99.08197

				171.11		99.08197

				171.13		99.07791

				171.16		99.07385

				171.18		99.07385

				171.2		99.07385

				171.22		99.07385

				171.24		99.07385

				171.26		99.06979

				171.28		99.06979

				171.3		99.06979

				171.32		99.06572

				171.35		99.06572

				171.37		99.06166

				171.39		99.0576

				171.41		99.0576

				171.43		99.05354

				171.45		99.05354

				171.47		99.05354

				171.49		99.05354

				171.51		99.04948

				171.53		99.04541

				171.56		99.04541

				171.58		99.04541

				171.6		99.04135

				171.62		99.03729

				171.64		99.03729

				171.66		99.02917

				171.68		99.0251

				171.7		99.02104

				171.72		99.01698

				171.74		99.01698

				171.77		99.01292

				171.79		99.01292

				171.81		99.00886

				171.83		99.00479

				171.85		99.00479

				171.87		99.00073

				171.89		98.99667

				171.91		98.99261

				171.93		98.98854

				171.95		98.98448

				171.98		98.98042

				172		98.98042

				172.02		98.9723

				172.04		98.96823

				172.06		98.96823

				172.08		98.96417

				172.1		98.96011

				172.12		98.95605

				172.14		98.95605

				172.16		98.95199

				172.19		98.94792

				172.21		98.94386

				172.23		98.94386

				172.25		98.94386

				172.27		98.9398

				172.29		98.9398

				172.31		98.9398

				172.33		98.93574

				172.35		98.93574

				172.38		98.93168

				172.4		98.93168

				172.42		98.93168

				172.44		98.92761

				172.46		98.92761

				172.48		98.92761

				172.5		98.92355

				172.52		98.92355

				172.54		98.92355

				172.56		98.92355

				172.59		98.91949

				172.61		98.91949

				172.63		98.91543

				172.65		98.91543

				172.67		98.91137

				172.69		98.91137

				172.71		98.9073

				172.73		98.90324

				172.75		98.89918

				172.77		98.89918

				172.8		98.89106

				172.82		98.89106

				172.84		98.89106

				172.86		98.88699

				172.88		98.88293

				172.9		98.88293

				172.92		98.87481

				172.94		98.87481

				172.96		98.87074

				172.98		98.87074

				173.01		98.86262

				173.03		98.86262

				173.05		98.85856

				173.07		98.8545

				173.09		98.8545

				173.11		98.85043

				173.13		98.84637

				173.15		98.84231

				173.17		98.84231

				173.19		98.83825

				173.22		98.83419

				173.24		98.83012

				173.26		98.83012

				173.28		98.82606

				173.3		98.82606

				173.32		98.822

				173.34		98.822

				173.36		98.822

				173.38		98.81794

				173.4		98.81794

				173.42		98.81388

				173.45		98.81388

				173.47		98.80981

				173.49		98.80575

				173.51		98.80575

				173.53		98.80575

				173.55		98.80575

				173.57		98.80575

				173.59		98.80169

				173.61		98.79763

				173.63		98.79357

				173.66		98.7895

				173.68		98.78544

				173.7		98.78138

				173.72		98.77732

				173.74		98.77326

				173.76		98.76919

				173.78		98.76513

				173.8		98.76107

				173.82		98.76107

				173.84		98.75701

				173.87		98.75701

				173.89		98.75294

				173.91		98.74482

				173.93		98.74076

				173.95		98.74076

				173.97		98.7367

				173.99		98.73263

				174.01		98.72857

				174.03		98.72451

				174.05		98.72045

				174.08		98.72045

				174.1		98.72045

				174.12		98.71639

				174.14		98.71639

				174.16		98.71639

				174.18		98.71232

				174.2		98.70826

				174.22		98.7042

				174.24		98.7042

				174.26		98.7042

				174.29		98.7042

				174.31		98.7042

				174.33		98.70014

				174.35		98.70014

				174.37		98.69608

				174.39		98.69608

				174.41		98.69201

				174.43		98.69201

				174.45		98.68795

				174.48		98.68795

				174.5		98.67983

				174.52		98.67577

				174.54		98.6717

				174.56		98.6717

				174.58		98.66764

				174.6		98.66764

				174.62		98.65952

				174.64		98.65546

				174.66		98.65139

				174.68		98.64733

				174.71		98.64327

				174.73		98.64327

				174.75		98.63515

				174.77		98.63515

				174.79		98.63108

				174.81		98.62702

				174.83		98.62296

				174.85		98.62296

				174.87		98.6189

				174.89		98.6189

				174.92		98.61077

				174.94		98.61077

				174.96		98.60671

				174.98		98.60671

				175		98.60265

				175.02		98.60265

				175.04		98.59859

				175.06		98.59859

				175.08		98.59452

				175.1		98.59046

				175.13		98.5864

				175.15		98.5864

				175.17		98.5864

				175.19		98.58234

				175.21		98.57828

				175.23		98.57421

				175.25		98.57015

				175.27		98.57015

				175.29		98.56609

				175.31		98.56203

				175.34		98.56203

				175.36		98.55797

				175.38		98.55797

				175.4		98.5539

				175.42		98.5539

				175.44		98.54984

				175.46		98.54578

				175.48		98.54172

				175.5		98.54172

				175.52		98.53766

				175.55		98.53359

				175.57		98.52953

				175.59		98.52547

				175.61		98.52141

				175.63		98.52141

				175.65		98.51328

				175.67		98.50922

				175.69		98.50922

				175.71		98.50516

				175.73		98.5011

				175.76		98.49703

				175.78		98.48891

				175.8		98.48891

				175.82		98.48485

				175.84		98.48079

				175.86		98.48079

				175.88		98.47672

				175.9		98.47266

				175.92		98.47266

				175.95		98.4686

				175.97		98.46454

				175.99		98.46048

				176.01		98.45641

				176.03		98.45641

				176.05		98.45641

				176.07		98.44829

				176.09		98.44829

				176.11		98.44423

				176.13		98.44017

				176.16		98.4361

				176.18		98.43204

				176.2		98.42798

				176.22		98.42798

				176.24		98.42392

				176.26		98.42392

				176.28		98.41986

				176.3		98.41579

				176.32		98.41173

				176.34		98.41173

				176.37		98.40361

				176.39		98.40361

				176.41		98.39955

				176.43		98.39548

				176.45		98.39142

				176.47		98.39548

				176.49		98.39142

				176.51		98.39142

				176.53		98.38736

				176.55		98.3833

				176.58		98.37923

				176.6		98.37923

				176.62		98.37111

				176.64		98.37111

				176.66		98.36299

				176.68		98.36299

				176.7		98.35892

				176.72		98.35892

				176.74		98.35486

				176.76		98.35486

				176.79		98.3508

				176.81		98.34268

				176.83		98.33861

				176.85		98.33455

				176.87		98.33455

				176.89		98.33049

				176.91		98.32643

				176.93		98.32237

				176.95		98.3183

				176.97		98.31424

				177		98.31424

				177.02		98.31018

				177.04		98.30612

				177.06		98.30206

				177.08		98.29393

				177.1		98.29393

				177.12		98.28987

				177.14		98.28987

				177.16		98.28581

				177.18		98.28581

				177.2		98.28581

				177.23		98.28175

				177.25		98.28175

				177.27		98.27362

				177.29		98.27362

				177.31		98.26956

				177.33		98.2655

				177.35		98.26143

				177.37		98.25737

				177.39		98.25737

				177.41		98.25331

				177.44		98.24925

				177.46		98.24519

				177.48		98.24519

				177.5		98.23706

				177.52		98.233

				177.54		98.22894

				177.56		98.22488

				177.58		98.22488

				177.6		98.22081

				177.62		98.22081

				177.65		98.21675

				177.67		98.20863

				177.69		98.20863

				177.71		98.20457

				177.73		98.2005

				177.75		98.2005

				177.77		98.19644

				177.79		98.18832

				177.81		98.18832

				177.83		98.18832

				177.86		98.18426

				177.88		98.18019

				177.9		98.17613

				177.92		98.16801

				177.94		98.16395

				177.96		98.16395

				177.98		98.16395

				178		98.15988

				178.02		98.15988

				178.04		98.15582

				178.06		98.1477

				178.09		98.1477

				178.11		98.14363

				178.13		98.14363

				178.15		98.13957

				178.17		98.13551

				178.19		98.13145

				178.21		98.13145

				178.23		98.13145

				178.25		98.12739

				178.27		98.12332

				178.3		98.1152

				178.32		98.11114

				178.34		98.11114

				178.36		98.11114

				178.38		98.10301

				178.4		98.10301

				178.42		98.09489

				178.44		98.08677

				178.46		98.0827

				178.48		98.0827

				178.51		98.07864

				178.53		98.07458

				178.55		98.07052

				178.57		98.06646

				178.59		98.06239

				178.61		98.05833

				178.63		98.05427

				178.65		98.05833

				178.67		98.05427

				178.69		98.05427

				178.72		98.05021

				178.74		98.05021

				178.76		98.04615

				178.78		98.04208

				178.8		98.03396

				178.82		98.03802

				178.84		98.03802

				178.86		98.0299

				178.88		98.02583

				178.9		98.02177

				178.93		98.01365

				178.95		98.00552

				178.97		97.9974

				178.99		97.9974

				179.01		97.99334

				179.03		97.98928

				179.05		97.98521

				179.07		97.98115

				179.09		97.97303

				179.11		97.96897

				179.13		97.96897

				179.16		97.9649

				179.18		97.96084

				179.2		97.96084

				179.22		97.95272

				179.24		97.95678

				179.26		97.94866

				179.28		97.94866

				179.3		97.94459

				179.32		97.94459

				179.34		97.94053

				179.37		97.94053

				179.39		97.93647

				179.41		97.93647

				179.43		97.93241

				179.45		97.92835

				179.47		97.92428

				179.49		97.92428

				179.51		97.91616

				179.53		97.9121

				179.55		97.9121

				179.58		97.90397

				179.6		97.89991

				179.62		97.89585

				179.64		97.89179

				179.66		97.88772

				179.68		97.88366

				179.7		97.8796

				179.72		97.87554

				179.74		97.87148

				179.76		97.86741

				179.79		97.86741

				179.81		97.86335

				179.83		97.85929

				179.85		97.85523

				179.87		97.85117

				179.89		97.8471

				179.91		97.84304

				179.93		97.84304

				179.95		97.83898

				179.97		97.83898

				180		97.83898

				180.02		97.83492

				180.04		97.83086

				180.06		97.82679

				180.08		97.82679

				180.1		97.82679

				180.12		97.81867

				180.14		97.81461

				180.16		97.81055

				180.18		97.81055

				180.21		97.80242

				180.23		97.79836

				180.25		97.79023

				180.27		97.78617

				180.29		97.77805

				180.31		97.77805

				180.33		97.77399

				180.35		97.76586

				180.37		97.76586

				180.39		97.7618

				180.42		97.75774

				180.44		97.74961

				180.46		97.74961

				180.48		97.74555

				180.5		97.74555

				180.52		97.74149

				180.54		97.73743

				180.56		97.7293

				180.58		97.72524

				180.6		97.72118

				180.62		97.71712

				180.65		97.71306

				180.67		97.70493

				180.69		97.70087

				180.71		97.69275

				180.73		97.68462

				180.75		97.6765

				180.77		97.6765

				180.79		97.66431

				180.81		97.66431

				180.83		97.66025

				180.86		97.65619

				180.88		97.65212

				180.9		97.65212

				180.92		97.644

				180.94		97.63994

				180.96		97.63994

				180.98		97.63588

				181		97.63181

				181.02		97.63181

				181.04		97.62775

				181.07		97.62775

				181.09		97.62369

				181.11		97.61963

				181.13		97.61557

				181.15		97.61557

				181.17		97.6115

				181.19		97.60744

				181.21		97.60338

				181.23		97.59932

				181.25		97.59526

				181.28		97.59119

				181.3		97.58713

				181.32		97.58713

				181.34		97.57901

				181.36		97.57495

				181.38		97.57088

				181.4		97.56682

				181.42		97.5587

				181.44		97.55463

				181.46		97.54651

				181.48		97.54245

				181.51		97.53432

				181.53		97.53432

				181.55		97.5262

				181.57		97.52214

				181.59		97.51808

				181.61		97.51401

				181.63		97.50995

				181.65		97.50995

				181.67		97.50183

				181.69		97.50183

				181.72		97.48964

				181.74		97.48964

				181.76		97.48152

				181.78		97.48152

				181.8		97.47746

				181.82		97.47339

				181.84		97.46933

				181.86		97.46527

				181.88		97.45715

				181.9		97.45715

				181.93		97.44902

				181.95		97.44902

				181.97		97.43683

				181.99		97.43683

				182.01		97.42465

				182.03		97.42465

				182.05		97.41652

				182.07		97.41246

				182.09		97.4084

				182.11		97.40434

				182.14		97.40028

				182.16		97.40028

				182.18		97.39621

				182.2		97.39621

				182.22		97.39215

				182.24		97.39215

				182.26		97.38809

				182.28		97.38403

				182.3		97.37997

				182.32		97.37997

				182.34		97.37184

				182.37		97.36778

				182.39		97.36372

				182.41		97.35966

				182.43		97.35559

				182.45		97.35153

				182.47		97.34341

				182.49		97.33935

				182.51		97.33528

				182.53		97.33122

				182.55		97.31903

				182.58		97.31903

				182.6		97.31497

				182.62		97.31091

				182.64		97.30685

				182.66		97.30279

				182.68		97.30279

				182.7		97.29872

				182.72		97.2906

				182.74		97.2906

				182.76		97.28248

				182.79		97.27841

				182.81		97.27841

				182.83		97.27841

				182.85		97.27435

				182.87		97.27029

				182.89		97.26623

				182.91		97.26217

				182.93		97.2581

				182.95		97.26217

				182.97		97.25404

				183		97.25404

				183.02		97.24998

				183.04		97.24186

				183.06		97.23373

				183.08		97.22561

				183.1		97.22155

				183.12		97.21342

				183.14		97.2053

				183.16		97.20123

				183.18		97.18905

				183.21		97.18092

				183.23		97.18092

				183.25		97.1728

				183.27		97.16874

				183.29		97.16468

				183.31		97.16468

				183.33		97.15655

				183.35		97.15655

				183.37		97.14843

				183.39		97.14437

				183.42		97.14437

				183.44		97.14437

				183.46		97.13624

				183.48		97.13218

				183.5		97.12812

				183.52		97.11999

				183.54		97.11187

				183.56		97.10375

				183.58		97.10375

				183.6		97.09562

				183.63		97.09156

				183.65		97.0875

				183.67		97.07937

				183.69		97.07531

				183.71		97.07125

				183.73		97.06719

				183.75		97.06719

				183.77		97.05906

				183.79		97.05906

				183.81		97.05094

				183.83		97.04688

				183.86		97.04281

				183.88		97.03875

				183.9		97.02657

				183.92		97.02657

				183.94		97.0225

				183.96		97.01438

				183.98		97.01438

				184		97.01438

				184.02		97.01032

				184.04		97.01032

				184.07		97.00626

				184.09		97.00626

				184.11		97.00219

				184.13		96.99813

				184.15		96.99407

				184.17		96.98595

				184.19		96.98188

				184.21		96.97782

				184.23		96.97376

				184.25		96.96157

				184.28		96.96157

				184.3		96.95345

				184.32		96.94939

				184.34		96.94126

				184.36		96.9372

				184.38		96.93314

				184.4		96.92908

				184.42		96.92501

				184.44		96.92095

				184.46		96.91283

				184.48		96.91283

				184.51		96.9047

				184.53		96.90064

				184.55		96.89658

				184.57		96.89252

				184.59		96.88846

				184.61		96.88033

				184.63		96.88033

				184.65		96.87221

				184.67		96.86408

				184.69		96.86408

				184.72		96.85596

				184.74		96.84783

				184.76		96.83971

				184.78		96.83565

				184.8		96.83159

				184.82		96.82346

				184.84		96.8194

				184.86		96.81534

				184.88		96.81128

				184.9		96.81128

				184.92		96.80315

				184.95		96.79909

				184.97		96.79503

				184.99		96.79097

				185.01		96.78284

				185.03		96.78284

				185.05		96.77878

				185.07		96.77472

				185.09		96.77066

				185.11		96.75847

				185.13		96.76659

				185.16		96.76253

				185.18		96.75847

				185.2		96.75441

				185.22		96.75035

				185.24		96.75035

				185.26		96.74222

				185.28		96.7341

				185.3		96.7341

				185.32		96.72191

				185.34		96.71785

				185.36		96.70972

				185.39		96.71379

				185.41		96.70566

				185.43		96.69348

				185.45		96.69348

				185.47		96.68535

				185.49		96.67723

				185.51		96.67723

				185.53		96.66504

				185.55		96.6691

				185.57		96.66098

				185.6		96.65692

				185.62		96.65286

				185.64		96.65286

				185.66		96.65286

				185.68		96.64473

				185.7		96.63661

				185.72		96.63255

				185.74		96.62036

				185.76		96.61223

				185.78		96.60411

				185.8		96.60411

				185.83		96.59192

				185.85		96.58786

				185.87		96.58786

				185.89		96.5838

				185.91		96.57568

				185.93		96.56755

				185.95		96.56349

				185.97		96.55943

				185.99		96.54724

				186.01		96.54318

				186.04		96.53912

				186.06		96.53099

				186.08		96.52693

				186.1		96.51881

				186.12		96.51881

				186.14		96.51475

				186.16		96.50662

				186.18		96.50662

				186.2		96.4985

				186.22		96.49443

				186.24		96.49037

				186.27		96.48225

				186.29		96.48225

				186.31		96.47819

				186.33		96.47006

				186.35		96.466

				186.37		96.45788

				186.39		96.45381

				186.41		96.44569

				186.43		96.44163

				186.45		96.4335

				186.48		96.42538

				186.5		96.42132

				186.52		96.41319

				186.54		96.40913

				186.56		96.40507

				186.58		96.39695

				186.6		96.39288

				186.62		96.38882

				186.64		96.38476

				186.66		96.37663

				186.68		96.36851

				186.71		96.36445

				186.73		96.35632

				186.75		96.35226

				186.77		96.3482

				186.79		96.34414

				186.81		96.33601

				186.83		96.33601

				186.85		96.33195

				186.87		96.32789

				186.89		96.31977

				186.92		96.31164

				186.94		96.3157

				186.96		96.29946

				186.98		96.29946

				187		96.29133

				187.02		96.28727

				187.04		96.27915

				187.06		96.27915

				187.08		96.27508

				187.1		96.27102

				187.13		96.25883

				187.15		96.25883

				187.17		96.25071

				187.19		96.24665

				187.21		96.23852

				187.23		96.24259

				187.25		96.2304

				187.27		96.22634

				187.29		96.22228

				187.31		96.21821

				187.34		96.21009

				187.36		96.20603

				187.38		96.19384

				187.4		96.18978

				187.42		96.17759

				187.44		96.17353

				187.46		96.16541

				187.48		96.16135

				187.5		96.15322

				187.52		96.14916

				187.54		96.14104

				187.57		96.13697

				187.59		96.12885

				187.61		96.12072

				187.63		96.1126

				187.65		96.1126

				187.67		96.10448

				187.69		96.09635

				187.71		96.09635

				187.73		96.08417

				187.75		96.08417

				187.78		96.0801

				187.8		96.07198

				187.82		96.06386

				187.84		96.05573

				187.86		96.05167

				187.88		96.04761

				187.9		96.03948

				187.92		96.03542

				187.94		96.03136

				187.96		96.0273

				187.99		96.0273

				188.01		96.02324

				188.03		96.01917

				188.05		96.01105

				188.07		96.00699

				188.09		96.00292

				188.11		96.00292

				188.13		95.9948

				188.15		95.98668

				188.17		95.97855

				188.2		95.97449

				188.22		95.96637

				188.24		95.9623

				188.26		95.95418

				188.28		95.94606

				188.3		95.93387

				188.32		95.92981

				188.34		95.92168

				188.36		95.91762

				188.38		95.9095

				188.4		95.90137

				188.43		95.89731

				188.45		95.89731

				188.47		95.88919

				188.49		95.88919

				188.51		95.88512

				188.53		95.88512

				188.55		95.877

				188.57		95.87294

				188.59		95.86888

				188.61		95.86888

				188.64		95.85263

				188.66		95.8445

				188.68		95.83638

				188.7		95.82826

				188.72		95.81607

				188.74		95.80795

				188.76		95.80795

				188.78		95.79982

				188.8		95.79576

				188.82		95.79982

				188.85		95.7917

				188.87		95.78764

				188.89		95.78357

				188.91		95.77139

				188.93		95.76732

				188.95		95.7592

				188.97		95.74701

				188.99		95.74701

				189.01		95.73889

				189.03		95.73077

				189.06		95.7267

				189.08		95.71858

				189.1		95.71858

				189.12		95.70639

				189.14		95.70639

				189.16		95.69827

				189.18		95.69421

				189.2		95.68608

				189.22		95.68202

				189.24		95.67796

				189.26		95.6739

				189.29		95.66171

				189.31		95.65765

				189.33		95.64952

				189.35		95.6414

				189.37		95.63328

				189.39		95.62921

				189.41		95.62515

				189.43		95.61703

				189.45		95.6089

				189.47		95.6089

				189.5		95.59672

				189.52		95.59266

				189.54		95.58047

				189.56		95.56828

				189.58		95.56422

				189.6		95.5561

				189.62		95.54391

				189.64		95.54391

				189.66		95.53579

				189.68		95.52766

				189.71		95.52766

				189.73		95.51548

				189.75		95.51548

				189.77		95.50735

				189.79		95.50329

				189.81		95.49517

				189.83		95.49517

				189.85		95.48704

				189.87		95.48298

				189.89		95.47892

				189.91		95.47486

				189.94		95.46673

				189.96		95.46267

				189.98		95.44236

				190		95.44236

				190.02		95.43017

				190.04		95.41799

				190.06		95.41799

				190.08		95.41392

				190.1		95.4058

				190.12		95.40986

				190.15		95.39768

				190.17		95.39361

				190.19		95.38955

				190.21		95.37737

				190.23		95.36924

				190.25		95.36518

				190.27		95.35299

				190.29		95.35299

				190.31		95.34487

				190.33		95.34081

				190.36		95.33268

				190.38		95.32862

				190.4		95.32456

				190.42		95.32456

				190.44		95.31644

				190.46		95.31237

				190.48		95.30831

				190.5		95.30019

				190.52		95.29206

				190.54		95.28394

				190.56		95.27175

				190.59		95.26769

				190.61		95.25957

				190.63		95.25144

				190.65		95.23926

				190.67		95.23519

				190.69		95.23113

				190.71		95.22301

				190.73		95.21488

				190.75		95.20676

				190.77		95.19864

				190.8		95.19864

				190.82		95.18645

				190.84		95.18239

				190.86		95.1702

				190.88		95.1702

				190.9		95.16208

				190.92		95.15801

				190.94		95.14583

				190.96		95.14177

				190.98		95.12958

				191		95.12958

				191.03		95.12146

				191.05		95.11333

				191.07		95.10521

				191.09		95.10115

				191.11		95.08896

				191.13		95.0849

				191.15		95.08084

				191.17		95.07677

				191.19		95.07271

				191.21		95.06865

				191.24		95.05646

				191.26		95.05646

				191.28		95.0524

				191.3		95.04021

				191.32		95.03209

				191.34		95.02397

				191.36		95.0199

				191.38		95.01584

				191.4		95.00772

				191.42		94.99553

				191.45		94.99147

				191.47		94.98741

				191.49		94.97928

				191.51		94.9671

				191.53		94.96304

				191.55		94.95897

				191.57		94.94679

				191.59		94.9346

				191.61		94.93054

				191.63		94.92648

				191.65		94.91835

				191.68		94.91023

				191.7		94.89804

				191.72		94.89398

				191.74		94.88586

				191.76		94.87367

				191.78		94.86555

				191.8		94.86148

				191.82		94.85742

				191.84		94.8493

				191.86		94.84117

				191.89		94.84117

				191.91		94.83305

				191.93		94.82899

				191.95		94.82492

				191.97		94.81274

				191.99		94.80461

				192.01		94.79649

				192.03		94.79243

				192.05		94.78024

				192.07		94.76806

				192.1		94.75993

				192.12		94.75181

				192.14		94.73962

				192.16		94.73962

				192.18		94.7315

				192.2		94.72744

				192.22		94.72337

				192.24		94.71931

				192.26		94.71525

				192.28		94.71525

				192.31		94.70306

				192.33		94.69494

				192.35		94.69088

				192.37		94.67869

				192.39		94.67057

				192.41		94.65838

				192.43		94.64619

				192.45		94.64213

				192.47		94.62995

				192.49		94.62182

				192.52		94.62182

				192.54		94.60964

				192.56		94.60557

				192.58		94.60151

				192.6		94.59339

				192.62		94.58932

				192.64		94.5812

				192.66		94.56901

				192.68		94.56495

				192.7		94.55683

				192.73		94.5487

				192.75		94.54058

				192.77		94.53246

				192.79		94.52433

				192.81		94.52027

				192.83		94.50808

				192.85		94.49996

				192.87		94.49184

				192.89		94.48777

				192.91		94.47152

				192.93		94.4634

				192.96		94.45934

				192.98		94.45528

				193		94.44715

				193.02		94.44309

				193.04		94.43497

				193.06		94.43497

				193.08		94.42684

				193.1		94.42684

				193.12		94.41466

				193.14		94.40653

				193.16		94.39841

				193.19		94.39435

				193.21		94.38622

				193.23		94.3781

				193.25		94.36591

				193.27		94.36185

				193.29		94.35779

				193.31		94.3456

				193.33		94.32935

				193.35		94.32935

				193.37		94.31717

				193.4		94.30904

				193.42		94.30092

				193.44		94.28873

				193.46		94.28467

				193.48		94.28467

				193.5		94.26842

				193.52		94.26436

				193.54		94.2603

				193.56		94.25624

				193.58		94.25217

				193.61		94.24405

				193.63		94.23592

				193.65		94.23592

				193.67		94.22374

				193.69		94.21155

				193.71		94.20343

				193.73		94.1953

				193.75		94.17499

				193.77		94.17093

				193.79		94.16281

				193.82		94.15875

				193.84		94.15062

				193.86		94.1425

				193.88		94.13437

				193.9		94.13437

				193.92		94.12625

				193.94		94.11406

				193.96		94.10188

				193.98		94.09781

				194		94.08563

				194.03		94.0775

				194.05		94.06532

				194.07		94.05719

				194.09		94.04501

				194.11		94.04501

				194.13		94.03688

				194.15		94.03282

				194.17		94.02064

				194.19		94.01251

				194.21		94.00439

				194.23		94.00032

				194.26		93.9922

				194.28		93.98814

				194.3		93.9922

				194.32		93.98814

				194.34		93.97189

				194.36		93.95564

				194.38		93.94752

				194.4		93.93939

				194.42		93.92721

				194.44		93.91908

				194.47		93.92315

				194.49		93.90284

				194.51		93.90284

				194.53		93.89877

				194.55		93.89065

				194.57		93.8744

				194.59		93.8744

				194.61		93.85003

				194.63		93.8419

				194.65		93.82972

				194.68		93.82566

				194.7		93.81347

				194.72		93.80941

				194.74		93.79722

				194.76		93.79316

				194.78		93.78504

				194.8		93.78097

				194.82		93.77691

				194.84		93.76879

				194.86		93.76066

				194.89		93.74848

				194.91		93.73629

				194.93		93.73223

				194.95		93.72004

				194.97		93.71192

				194.99		93.71598

				195.01		93.71192

				195.03		93.69567

				195.05		93.67536

				195.07		93.67942

				195.1		93.65911

				195.12		93.64286

				195.14		93.6388

				195.16		93.64693

				195.18		93.62661

				195.2		93.61849

				195.22		93.61849

				195.24		93.61037

				195.26		93.59412

				195.28		93.58193

				195.31		93.57787

				195.33		93.56568

				195.35		93.55756

				195.37		93.54944

				195.39		93.54537

				195.41		93.54131

				195.43		93.53319

				195.45		93.52506

				195.47		93.51694

				195.49		93.50475

				195.51		93.49257

				195.54		93.48038

				195.56		93.46413

				195.58		93.46819

				195.6		93.46007

				195.62		93.44788

				195.64		93.44788

				195.66		93.44788

				195.68		93.43164

				195.7		93.41945

				195.72		93.41133

				195.75		93.39508

				195.77		93.38289

				195.79		93.3707

				195.81		93.36664

				195.83		93.36258

				195.85		93.35852

				195.87		93.35039

				195.89		93.34633

				195.91		93.33821

				195.93		93.32602

				195.96		93.31384

				195.98		93.30165

				196		93.2854

				196.02		93.27728

				196.04		93.26915

				196.06		93.26103

				196.08		93.26103

				196.1		93.24884

				196.12		93.24478

				196.14		93.23259

				196.17		93.22853

				196.19		93.21228

				196.21		93.21228

				196.23		93.20416

				196.25		93.2001

				196.27		93.18385

				196.29		93.17573

				196.31		93.1676

				196.33		93.15541

				196.35		93.14323

				196.38		93.13104

				196.4		93.11886

				196.42		93.10667

				196.44		93.09855

				196.46		93.09448

				196.48		93.09042

				196.5		93.09042

				196.52		93.07417

				196.54		93.07011

				196.56		93.06199

				196.58		93.0498

				196.61		93.04168

				196.63		93.03761

				196.65		93.02543

				196.67		93.0173

				196.69		93.00106

				196.71		92.99293

				196.73		92.98481

				196.75		92.96856

				196.77		92.96044

				196.79		92.95637

				196.82		92.93606

				196.84		92.932

				196.86		92.932

				196.88		92.91981

				196.9		92.91169

				196.92		92.91169

				196.94		92.8995

				196.96		92.89138

				196.98		92.88326

				197		92.87919

				197.03		92.86701

				197.05		92.86295

				197.07		92.85076

				197.09		92.85482

				197.11		92.84264

				197.13		92.83857

				197.15		92.83045

				197.17		92.81826

				197.19		92.79795

				197.21		92.79389

				197.24		92.77358

				197.26		92.76952

				197.28		92.76546

				197.3		92.75327

				197.32		92.73702

				197.34		92.73702

				197.36		92.71265

				197.38		92.70046

				197.4		92.68828

				197.42		92.68421

				197.45		92.67609

				197.47		92.67609

				197.49		92.66797

				197.51		92.6639

				197.53		92.65172

				197.55		92.63547

				197.57		92.61922

				197.59		92.61516

				197.61		92.59485

				197.64		92.59891

				197.66		92.58673

				197.68		92.5786

				197.7		92.57048

				197.72		92.56641

				197.74		92.5461

				197.76		92.5461

				197.78		92.52986

				197.8		92.51767

				197.82		92.50548

				197.85		92.50955

				197.87		92.4933

				197.89		92.48111

				197.91		92.46893

				197.93		92.46486

				197.95		92.44455

				197.97		92.44049

				197.99		92.44049

				198.01		92.4283

				198.03		92.42424

				198.06		92.41612

				198.08		92.40393

				198.1		92.39581

				198.12		92.38768

				198.14		92.3755

				198.16		92.36331

				198.18		92.35925

				198.2		92.343

				198.22		92.33488

				198.24		92.32269

				198.27		92.32269

				198.29		92.30644

				198.31		92.29832

				198.33		92.27395

				198.35		92.27395

				198.37		92.2577

				198.39		92.25364

				198.41		92.24551

				198.43		92.24551

				198.45		92.22926

				198.48		92.2252

				198.5		92.21301

				198.52		92.20083

				198.54		92.1927

				198.56		92.18458

				198.58		92.17239

				198.6		92.15208

				198.62		92.14802

				198.64		92.13177

				198.66		92.11553

				198.69		92.10334

				198.71		92.09521

				198.73		92.08303

				198.75		92.07897

				198.77		92.06678

				198.79		92.05866

				198.81		92.05866

				198.83		92.04647

				198.85		92.03428

				198.87		92.02616

				198.9		92.0221

				198.92		92.00585

				198.94		92.00585

				198.96		91.99773

				198.98		91.98554

				199		91.97741

				199.02		91.96117

				199.04		91.94898

				199.06		91.94086

				199.08		91.93679

				199.11		91.92867

				199.13		91.92055

				199.15		91.9043

				199.17		91.89211

				199.19		91.87993

				199.21		91.86774

				199.23		91.85555

				199.25		91.85555

				199.27		91.84337

				199.29		91.83118

				199.32		91.81899

				199.34		91.81087

				199.36		91.79462

				199.38		91.7865

				199.4		91.77025

				199.42		91.76213

				199.44		91.74588

				199.46		91.73775

				199.48		91.72963

				199.5		91.71744

				199.53		91.70526

				199.55		91.71338

				199.57		91.69713

				199.59		91.68495

				199.61		91.67276

				199.63		91.65651

				199.65		91.64026

				199.67		91.63214

				199.69		91.61589

				199.71		91.60777

				199.74		91.60777

				199.76		91.6037

				199.78		91.6037

				199.8		91.59152

				199.82		91.59152

				199.84		91.57933

				199.86		91.56308

				199.88		91.55496

				199.9		91.55496

				199.92		91.53871

				199.95		91.53059

				199.97		91.52246

				199.99		91.50621

				200.01		91.4859

				200.03		91.47372

				200.05		91.46559

				200.07		91.46153

				200.09		91.45341

				200.11		91.44935

				200.13		91.44122

				200.16		91.42497

				200.18		91.41279

				200.2		91.40466

				200.22		91.39248

				200.24		91.37623

				200.26		91.37217

				200.28		91.35186

				200.3		91.33967

				200.32		91.33967

				200.34		91.32342

				200.37		91.31124

				200.39		91.30717

				200.41		91.29499

				200.43		91.27468

				200.45		91.27061

				200.47		91.26249

				200.49		91.24624

				200.51		91.23406

				200.53		91.22187

				200.55		91.20968

				200.57		91.20562

				200.6		91.19344

				200.62		91.18531

				200.64		91.17719

				200.66		91.165

				200.68		91.15688

				200.7		91.13657

				200.72		91.12438

				200.74		91.12438

				200.76		91.10813

				200.78		91.08782

				200.81		91.09188

				200.83		91.0797

				200.85		91.05939

				200.87		91.05126

				200.89		91.04314

				200.91		91.03502

				200.93		91.03502

				200.95		91.02689

				200.97		91.01877

				200.99		91.00252

				201.02		90.99033

				201.04		90.97815

				201.06		90.9619

				201.08		90.94971

				201.1		90.94971

				201.12		90.9294

				201.14		90.90909

				201.16		90.90503

				201.18		90.89284

				201.2		90.88472

				201.23		90.88066

				201.25		90.87253

				201.27		90.84816

				201.29		90.84004

				201.31		90.82379

				201.33		90.8116

				201.35		90.79942

				201.37		90.79535

				201.39		90.78317

				201.41		90.77098

				201.43		90.75879

				201.46		90.74661

				201.48		90.73442

				201.5		90.7263

				201.52		90.71005

				201.54		90.70599

				201.56		90.6938

				201.58		90.68568

				201.6		90.67755

				201.62		90.66537

				201.64		90.65318

				201.67		90.64099

				201.69		90.63287

				201.71		90.61662

				201.73		90.6085

				201.75		90.59631

				201.77		90.58819

				201.79		90.576

				201.81		90.56382

				201.83		90.54757

				201.85		90.53944

				201.88		90.53132

				201.9		90.51507

				201.92		90.49882

				201.94		90.4907

				201.96		90.47851

				201.98		90.46226

				202		90.46633

				202.02		90.46226

				202.04		90.44602

				202.06		90.43789

				202.08		90.4257

				202.11		90.41352

				202.13		90.39727

				202.15		90.38915

				202.17		90.36884

				202.19		90.35665

				202.21		90.3404

				202.23		90.3404

				202.25		90.32415

				202.27		90.32009

				202.29		90.31603

				202.32		90.30384

				202.34		90.28353

				202.36		90.27947

				202.38		90.26322

				202.4		90.25104

				202.42		90.24291

				202.44		90.23479

				202.46		90.2226

				202.48		90.21042

				202.5		90.19417

				202.53		90.17792

				202.55		90.16167

				202.57		90.14542

				202.59		90.14136

				202.61		90.12917

				202.63		90.11293

				202.65		90.11699

				202.67		90.09262

				202.69		90.08449

				202.71		90.07637

				202.73		90.0723

				202.76		90.04793

				202.78		90.04793

				202.8		90.02356

				202.82		90.00731

				202.84		89.99513

				202.86		89.99106

				202.88		89.97482

				202.9		89.97482

				202.92		89.95857

				202.94		89.95044

				202.97		89.92607

				202.99		89.91795

				203.01		89.9017

				203.03		89.9017

				203.05		89.88139

				203.07		89.88139

				203.09		89.86514

				203.11		89.85295

				203.13		89.84483

				203.15		89.8367

				203.18		89.81233

				203.2		89.81233

				203.22		89.79608

				203.24		89.77984

				203.26		89.76359

				203.28		89.75953

				203.3		89.74328

				203.32		89.73515

				203.34		89.71078

				203.36		89.71484

				203.39		89.69453

				203.41		89.68235

				203.43		89.67016

				203.45		89.67016

				203.47		89.63766

				203.49		89.6336

				203.51		89.61735

				203.53		89.60517

				203.55		89.59298

				203.57		89.58892

				203.6		89.56861

				203.62		89.56455

				203.64		89.5483

				203.66		89.54424

				203.68		89.53205

				203.7		89.52799

				203.72		89.51174

				203.74		89.50362

				203.76		89.47518

				203.78		89.46299

				203.81		89.45081

				203.83		89.43862

				203.85		89.4305

				203.87		89.43456

				203.89		89.42237

				203.91		89.41425

				203.93		89.398

				203.95		89.38988

				203.97		89.3655

				203.99		89.35738

				204.02		89.33707

				204.04		89.32895

				204.06		89.3127

				204.08		89.30457

				204.1		89.28833

				204.12		89.2802

				204.14		89.27208

				204.16		89.26395

				204.18		89.2477

				204.2		89.24364

				204.23		89.23146

				204.25		89.21115

				204.27		89.19896

				204.29		89.19084

				204.31		89.16646

				204.33		89.15022

				204.35		89.13803

				204.37		89.12178

				204.39		89.10147

				204.41		89.09335

				204.44		89.08116

				204.46		89.0771

				204.48		89.06085

				204.5		89.06085

				204.52		89.04866

				204.54		89.03648

				204.56		89.02023

				204.58		89.00804

				204.6		88.99586

				204.62		88.98773

				204.65		88.97148

				204.67		88.9593

				204.69		88.94305

				204.71		88.93493

				204.73		88.91868

				204.75		88.91055

				204.77		88.89837

				204.79		88.89024

				204.81		88.86993

				204.83		88.86587

				204.86		88.85368

				204.88		88.83337

				204.9		88.81306

				204.92		88.80088

				204.94		88.78057

				204.96		88.7765

				204.98		88.76838

				205		88.75619

				205.02		88.73995

				205.04		88.73995

				205.07		88.71964

				205.09		88.71151

				205.11		88.70339

				205.13		88.69933

				205.15		88.68714

				205.17		88.68308

				205.19		88.66277

				205.21		88.65871

				205.23		88.65058

				205.26		88.63433

				205.28		88.62215

				205.3		88.61402

				205.32		88.60184

				205.34		88.58559

				205.36		88.56934

				205.38		88.54903

				205.4		88.54091

				205.42		88.52466

				205.44		88.50028

				205.47		88.49622

				205.49		88.49216

				205.51		88.47185

				205.53		88.4556

				205.55		88.45154

				205.57		88.43529

				205.59		88.42717

				205.61		88.41498

				205.63		88.41092

				205.65		88.39873

				205.68		88.39061

				205.7		88.37842

				205.72		88.37436

				205.74		88.35405

				205.76		88.35405

				205.78		88.34186

				205.8		88.32562

				205.82		88.30937

				205.84		88.30124

				205.86		88.28093

				205.89		88.26875

				205.91		88.2525

				205.93		88.24031

				205.95		88.22406

				205.97		88.21594

				205.99		88.21188

				206.01		88.20782

				206.03		88.18751

				206.05		88.18344

				206.07		88.17938

				206.1		88.15501

				206.12		88.14688

				206.14		88.14282

				206.16		88.12657

				206.18		88.11033

				206.2		88.11439

				206.22		88.09408

				206.24		88.09408

				206.26		88.07783

				206.28		88.05752

				206.3		88.02908

				206.33		88.02096

				206.35		88.00065

				206.37		87.9844

				206.39		87.9844

				206.41		87.98034

				206.43		87.96409

				206.45		87.94378

				206.47		87.93566

				206.49		87.92347

				206.51		87.90316

				206.54		87.88691

				206.56		87.87473

				206.58		87.86254

				206.6		87.85035

				206.62		87.83817

				206.64		87.83004

				206.66		87.83004

				206.68		87.81786

				206.7		87.80567

				206.72		87.79348

				206.75		87.78536

				206.77		87.76911

				206.79		87.76099

				206.81		87.75286

				206.83		87.7488

				206.85		87.73662

				206.87		87.72443

				206.89		87.71631

				206.91		87.70818

				206.93		87.68787

				206.96		87.67568

				206.98		87.66756

				207		87.64319

				207.02		87.631

				207.04		87.62694

				207.06		87.61069

				207.08		87.59851

				207.1		87.59444

				207.12		87.58226

				207.14		87.56601

				207.17		87.55382

				207.19		87.54164

				207.21		87.53757

				207.23		87.52133

				207.25		87.52133

				207.27		87.51726

				207.29		87.50102

				207.31		87.47664

				207.33		87.46852

				207.35		87.44821

				207.37		87.43196

				207.4		87.42384

				207.42		87.42384

				207.44		87.41571

				207.46		87.40759

				207.48		87.3954

				207.5		87.38728

				207.52		87.37103

				207.54		87.35478

				207.56		87.34259

				207.58		87.33447

				207.61		87.31822

				207.63		87.30604

				207.65		87.29385

				207.67		87.28573

				207.69		87.26948

				207.71		87.25323

				207.73		87.24917

				207.75		87.24104

				207.77		87.22479

				207.79		87.20855

				207.82		87.1923

				207.84		87.18417

				207.86		87.16793

				207.88		87.16386

				207.9		87.15574

				207.92		87.1598

				207.94		87.14355

				207.96		87.13137

				207.98		87.11918

				208		87.10293

				208.03		87.08668

				208.05		87.0745

				208.07		87.06231

				208.09		87.04606

				208.11		87.03794

				208.13		87.02575

				208.15		87.02169

				208.17		87.00951

				208.19		86.99732

				208.21		86.98513

				208.24		86.97701

				208.26		86.96482

				208.28		86.94857

				208.3		86.94451

				208.32		86.93639

				208.34		86.9242

				208.36		86.90795

				208.38		86.89983

				208.4		86.87952

				208.42		86.86327

				208.45		86.84702

				208.47		86.83484

				208.49		86.81453

				208.51		86.8064

				208.53		86.79422

				208.55		86.78203

				208.57		86.76984

				208.59		86.76984

				208.61		86.75766

				208.63		86.74547

				208.66		86.74141

				208.68		86.72922

				208.7		86.71297

				208.72		86.69266

				208.74		86.68454

				208.76		86.67235

				208.78		86.66017

				208.8		86.65204

				208.82		86.64392

				208.84		86.62767

				208.87		86.61955

				208.89		86.61142

				208.91		86.59111

				208.93		86.59111

				208.95		86.58705

				208.97		86.57486

				208.99		86.55455

				209.01		86.55455

				209.03		86.53018

				209.05		86.51799

				209.08		86.49362

				209.1		86.48956

				209.12		86.46519

				209.14		86.45706

				209.16		86.44488

				209.18		86.44488

				209.2		86.42863

				209.22		86.42051

				209.24		86.41238

				209.26		86.40019

				209.29		86.38395

				209.31		86.38395

				209.33		86.36364

				209.35		86.35551

				209.37		86.34333

				209.39		86.3352

				209.41		86.29864

				209.43		86.29864

				209.45		86.28239

				209.47		86.26615

				209.5		86.24584

				209.52		86.2499

				209.54		86.22553

				209.56		86.22553

				209.58		86.2174

				209.6		86.2174

				209.62		86.20115

				209.64		86.20115

				209.66		86.16866

				209.68		86.15241

				209.71		86.12804

				209.73		86.12397

				209.75		86.0996

				209.77		86.0996

				209.79		86.08742

				209.81		86.07929

				209.83		86.05086

				209.85		86.05086

				209.87		86.03055

				209.89		86.02242

				209.92		86.00617

				209.94		86.00211

				209.96		85.9818

				209.98		85.96555

				210		85.94524

				210.02		85.94118

				210.04		85.92087

				210.06		85.91275

				210.08		85.90056

				210.1		85.90056

				210.12		85.88025

				210.15		85.87619

				210.17		85.85588

				210.19		85.84775

				210.21		85.83151

				210.23		85.82338

				210.25		85.79901

				210.27		85.79495

				210.29		85.78276

				210.31		85.76651

				210.33		85.7462

				210.36		85.7462

				210.38		85.72995

				210.4		85.72183

				210.42		85.71777

				210.44		85.70964

				210.46		85.68527

				210.48		85.67715

				210.5		85.65684

				210.52		85.64059

				210.54		85.63246

				210.57		85.62028

				210.59		85.59997

				210.61		85.58372

				210.63		85.56747

				210.65		85.55935

				210.67		85.54716

				210.69		85.53497

				210.71		85.53091

				210.73		85.51873

				210.75		85.49435

				210.78		85.48217

				210.8		85.47404

				210.82		85.4578

				210.84		85.44967

				210.86		85.44155

				210.88		85.4253

				210.9		85.41311

				210.92		85.40093

				210.94		85.39686

				210.96		85.37249

				210.99		85.36437

				211.01		85.34406

				211.03		85.32781

				211.05		85.30344

				211.07		85.29937

				211.09		85.27906

				211.11		85.275

				211.13		85.26688

				211.15		85.25875

				211.17		85.23844

				211.2		85.23032

				211.22		85.21407

				211.24		85.1897

				211.26		85.17345

				211.28		85.16533

				211.3		85.15314

				211.32		85.14908

				211.34		85.14502

				211.36		85.12471

				211.38		85.10846

				211.41		85.09221

				211.43		85.06784

				211.45		85.06784

				211.47		85.05159

				211.49		85.04753

				211.51		85.03128

				211.53		85.01503

				211.55		84.99066

				211.57		84.99066

				211.6		84.96222

				211.62		84.95816

				211.64		84.94597

				211.66		84.93379

				211.68		84.9216

				211.7		84.91754

				211.72		84.90535

				211.74		84.88911

				211.76		84.88098

				211.78		84.85661

				211.81		84.84036

				211.83		84.82005

				211.85		84.8038

				211.87		84.78349

				211.89		84.77537

				211.91		84.76318

				211.93		84.751

				211.95		84.73068

				211.97		84.72662

				211.99		84.71444

				212.02		84.69819

				212.04		84.68194

				212.06		84.67382

				212.08		84.64944

				212.1		84.62913

				212.12		84.61288

				212.14		84.60476

				212.16		84.59664

				212.18		84.58445

				212.2		84.57633

				212.23		84.56414

				212.25		84.55195

				212.27		84.53571

				212.29		84.52758

				212.31		84.5154

				212.33		84.49915

				212.35		84.49102

				212.37		84.47071

				212.39		84.45446

				212.41		84.44634

				212.44		84.43415

				212.46		84.41384

				212.48		84.40572

				212.5		84.38135

				212.52		84.36104

				212.54		84.34479

				212.56		84.3326

				212.58		84.31229

				212.6		84.31229

				212.62		84.29604

				212.65		84.28792

				212.67		84.27167

				212.69		84.26761

				212.71		84.2473

				212.73		84.23917

				212.75		84.21886

				212.77		84.2148

				212.79		84.19043

				212.81		84.18231

				212.83		84.17012

				212.86		84.15793

				212.88		84.12544

				212.9		84.11731

				212.92		84.097

				212.94		84.08075

				212.96		84.06857

				212.98		84.06451

				213		84.05232

				213.02		84.0442

				213.04		84.02388

				213.07		84.01576

				213.09		83.99545

				213.11		83.98733

				213.13		83.96295

				213.15		83.95077

				213.17		83.93046

				213.19		83.92233

				213.21		83.89796

				213.23		83.88984

				213.25		83.87765

				213.28		83.8614

				213.3		83.84109

				213.32		83.83297

				213.34		83.81672

				213.36		83.80047

				213.38		83.78422

				213.4		83.77204

				213.42		83.75173

				213.44		83.73954

				213.46		83.72329

				213.49		83.70704

				213.51		83.6908

				213.53		83.68267

				213.55		83.66236

				213.57		83.65017

				213.59		83.63393

				213.61		83.6258

				213.63		83.60143

				213.65		83.59331

				213.67		83.58112

				213.7		83.56487

				213.72		83.5405

				213.74		83.52831

				213.76		83.51613

				213.78		83.49582

				213.8		83.47957

				213.82		83.47144

				213.84		83.4552

				213.86		83.43895

				213.88		83.42676

				213.91		83.41457

				213.93		83.39426

				213.95		83.38614

				213.97		83.36583

				213.99		83.34552

				214.01		83.32521

				214.03		83.31709

				214.05		83.29677

				214.07		83.28459

				214.09		83.26428

				214.12		83.25615

				214.14		83.23584

				214.16		83.22366

				214.18		83.20335

				214.2		83.19929

				214.22		83.17897

				214.24		83.16679

				214.26		83.16273

				214.28		83.14648

				214.31		83.13023

				214.33		83.12211

				214.35		83.09367

				214.37		83.07336

				214.39		83.06117

				214.41		83.04086

				214.43		83.01649

				214.45		83.00837

				214.47		82.984

				214.49		82.96775

				214.52		82.96369

				214.54		82.94744

				214.56		82.94337

				214.58		82.92713

				214.6		82.91494

				214.62		82.89869

				214.64		82.87838

				214.66		82.86213

				214.68		82.84995

				214.7		82.82964

				214.73		82.81339

				214.75		82.81339

				214.77		82.79308

				214.79		82.78089

				214.81		82.77277

				214.83		82.75652

				214.85		82.72809

				214.87		82.72402

				214.89		82.69559

				214.92		82.67528

				214.94		82.65497

				214.96		82.64684

				214.98		82.61841

				215		82.61029

				215.02		82.58997

				215.04		82.57779

				215.06		82.55748

				215.08		82.54529

				215.1		82.53311

				215.13		82.51686

				215.15		82.50061

				215.17		82.48436

				215.19		82.46405

				215.21		82.44374

				215.23		82.43562

				215.25		82.41937

				215.27		82.40312

				215.29		82.39093

				215.31		82.37875

				215.34		82.35844

				215.36		82.34219

				215.38		82.33406

				215.4		82.32188

				215.42		82.30563

				215.44		82.28126

				215.46		82.2772

				215.48		82.25689

				215.5		82.23657

				215.53		82.22033

				215.55		82.2122

				215.57		82.17971

				215.59		82.16752

				215.61		82.14315

				215.63		82.13502

				215.65		82.11065

				215.67		82.10659

				215.69		82.07815

				215.71		82.07815

				215.74		82.05784

				215.76		82.04566

				215.78		82.02535

				215.8		82.01316

				215.82		81.98879

				215.84		81.96848

				215.86		81.95223

				215.88		81.95223

				215.9		81.93192

				215.92		81.91973

				215.95		81.90755

				215.97		81.89942

				215.99		81.87099

				216.01		81.8588

				216.03		81.83849

				216.05		81.82224

				216.07		81.79787

				216.09		81.78569

				216.11		81.76131

				216.14		81.74913

				216.16		81.73694

				216.18		81.72882

				216.2		81.71257

				216.22		81.70444

				216.24		81.68413

				216.26		81.66382

				216.28		81.63539

				216.3		81.61914

				216.32		81.59883

				216.35		81.57852

				216.37		81.5704

				216.39		81.55821

				216.41		81.53384

				216.43		81.52165

				216.45		81.50946

				216.47		81.48509

				216.49		81.47291

				216.51		81.46478

				216.53		81.44447

				216.56		81.43229

				216.58		81.41604

				216.6		81.39979

				216.62		81.37948

				216.64		81.36323

				216.66		81.33886

				216.68		81.32667

				216.7		81.3023

				216.72		81.29824

				216.75		81.28199

				216.77		81.26168

				216.79		81.23731

				216.81		81.23324

				216.83		81.20481

				216.85		81.18856

				216.87		81.16825

				216.89		81.16013

				216.91		81.12763

				216.93		81.11544

				216.96		81.0992

				216.98		81.08295

				217		81.06264

				217.02		81.05045

				217.04		81.02608

				217.06		81.00983

				217.08		80.99764

				217.1		80.9814

				217.12		80.95296

				217.15		80.94484

				217.17		80.92859

				217.19		80.9164

				217.21		80.89203

				217.23		80.88391

				217.25		80.85953

				217.27		80.84735

				217.29		80.81891

				217.31		80.81079

				217.33		80.79048

				217.36		80.77423

				217.38		80.75798

				217.4		80.74173

				217.42		80.71736

				217.44		80.70518

				217.46		80.68486

				217.48		80.66455

				217.5		80.64831

				217.52		80.64424

				217.54		80.62393

				217.57		80.61175

				217.59		80.5955

				217.61		80.58738

				217.63		80.563

				217.65		80.55488

				217.67		80.54269

				217.69		80.52644

				217.71		80.49801

				217.73		80.48582

				217.76		80.46145

				217.78		80.43708

				217.8		80.41677

				217.82		80.40458

				217.84		80.38427

				217.86		80.36802

				217.88		80.34365

				217.9		80.3274

				217.92		80.31522

				217.94		80.29491

				217.97		80.27053

				217.99		80.26241

				218.01		80.2421

				218.03		80.22179

				218.05		80.20148

				218.07		80.19335

				218.09		80.17711

				218.11		80.16086

				218.13		80.14055

				218.15		80.12024

				218.18		80.09993

				218.2		80.06743

				218.22		80.039

				218.24		80.01869

				218.26		80.00244

				218.28		79.98619

				218.3		79.974

				218.32		79.96588

				218.34		79.95369

				218.36		79.94151

				218.39		79.9212

				218.41		79.90089

				218.43		79.89276

				218.45		79.87651

				218.47		79.8562

				218.49		79.83995

				218.51		79.82777

				218.53		79.79527

				218.55		79.78309

				218.57		79.76278

				218.6		79.74653

				218.62		79.73028

				218.64		79.71403

				218.66		79.68966

				218.68		79.66529

				218.7		79.64904

				218.72		79.62873

				218.74		79.60842

				218.76		79.59623

				218.78		79.58404

				218.81		79.55561

				218.83		79.5353

				218.85		79.51499

				218.87		79.49468

				218.89		79.46624

				218.91		79.45

				218.93		79.43375

				218.95		79.42156

				218.97		79.40125

				218.99		79.39313

				219.02		79.37688

				219.04		79.35657

				219.06		79.33626

				219.08		79.32813

				219.1		79.30376

				219.12		79.28751

				219.14		79.2672

				219.16		79.24283

				219.18		79.21846

				219.2		79.19815

				219.23		79.16971

				219.25		79.15346

				219.27		79.13722

				219.29		79.11691

				219.31		79.10066

				219.33		79.08441

				219.35		79.07629

				219.37		79.06004

				219.39		79.03566

				219.41		79.01535

				219.43		79.00317

				219.46		78.97473

				219.48		78.96255

				219.5		78.95036

				219.52		78.93818

				219.54		78.9138

				219.56		78.89755

				219.58		78.86912

				219.6		78.85287

				219.62		78.83256

				219.64		78.80819

				219.67		78.77975

				219.69		78.75944

				219.71		78.73101

				219.73		78.71476

				219.75		78.69445

				219.77		78.69039

				219.79		78.68227

				219.81		78.66195

				219.83		78.63758

				219.85		78.62133

				219.88		78.5929

				219.9		78.57259

				219.92		78.5604

				219.94		78.54822

				219.96		78.52384

				219.98		78.50353

				220		78.47916

				220.02		78.45885

				220.04		78.43448

				220.06		78.41417

				220.09		78.39386

				220.11		78.37761

				220.13		78.3573

				220.15		78.34105

				220.17		78.31668

				220.19		78.30449

				220.21		78.28418

				220.23		78.26793

				220.25		78.24356

				220.27		78.23544

				220.3		78.21107

				220.32		78.19482

				220.34		78.16638

				220.36		78.15013

				220.38		78.12576

				220.4		78.10545

				220.42		78.0892

				220.44		78.06889

				220.46		78.05264

				220.49		78.03233

				220.51		78.01202

				220.53		77.98765

				220.55		77.97547

				220.57		77.95515

				220.59		77.93078

				220.61		77.92266

				220.63		77.90641

				220.65		77.87798

				220.67		77.85767

				220.7		77.84548

				220.72		77.81298

				220.74		77.79673

				220.76		77.77642

				220.78		77.75611

				220.8		77.7358

				220.82		77.71955

				220.84		77.69112

				220.86		77.67487

				220.88		77.64644

				220.91		77.63019

				220.93		77.60988

				220.95		77.58957

				220.97		77.56926

				220.99		77.55301

				221.01		77.52458

				221.03		77.51239

				221.05		77.49614

				221.07		77.47177

				221.09		77.45146

				221.12		77.43927

				221.14		77.40678

				221.16		77.38647

				221.18		77.37022

				221.2		77.35397

				221.22		77.33772

				221.24		77.31741

				221.26		77.29304

				221.28		77.28085

				221.3		77.25242

				221.33		77.23211

				221.35		77.20773

				221.37		77.19555

				221.39		77.16711

				221.41		77.15899

				221.43		77.13462

				221.45		77.12649

				221.47		77.10618

				221.49		77.08181

				221.51		77.04931

				221.54		77.03307

				221.56		77.00869

				221.58		76.98026

				221.6		76.96401

				221.62		76.9437

				221.64		76.91933

				221.66		76.89495

				221.68		76.87871

				221.7		76.8584

				221.72		76.83402

				221.75		76.81371

				221.77		76.79747

				221.79		76.77309

				221.81		76.75684

				221.83		76.74872

				221.85		76.72435

				221.87		76.69998

				221.89		76.68373

				221.91		76.65935

				221.93		76.6228

				221.95		76.61061

				221.98		76.59436

				222		76.56593

				222.02		76.54562

				222.04		76.52937

				222.06		76.505

				222.08		76.48469

				222.1		76.46438

				222.12		76.44813

				222.14		76.42375

				222.16		76.39938

				222.19		76.37907

				222.21		76.36282

				222.23		76.33845

				222.25		76.3222

				222.27		76.30189

				222.29		76.27752

				222.31		76.25315

				222.33		76.24096

				222.35		76.20847

				222.37		76.19222

				222.4		76.16784

				222.42		76.1516

				222.44		76.13129

				222.46		76.1191

				222.48		76.09879

				222.5		76.08254

				222.52		76.05817

				222.54		76.0338

				222.56		76.00536

				222.58		75.98505

				222.61		75.95662

				222.63		75.93631

				222.65		75.916

				222.67		75.90381

				222.69		75.87944

				222.71		75.86725

				222.73		75.84694

				222.75		75.83069

				222.77		75.80632

				222.79		75.78601

				222.82		75.76164

				222.84		75.74133

				222.86		75.71289

				222.88		75.69258

				222.9		75.66821

				222.92		75.6479

				222.94		75.61134

				222.96		75.59916

				222.98		75.57478

				223		75.55447

				223.03		75.53822

				223.05		75.51791

				223.07		75.49354

				223.09		75.46917

				223.11		75.44886

				223.13		75.42855

				223.15		75.40824

				223.17		75.39199

				223.19		75.37574

				223.21		75.35137

				223.24		75.327

				223.26		75.31075

				223.28		75.28638

				223.3		75.26607

				223.32		75.24169

				223.34		75.21326

				223.36		75.18482

				223.38		75.15233

				223.4		75.12389

				223.42		75.10764

				223.45		75.08327

				223.47		75.06296

				223.49		75.04265

				223.51		75.03859

				223.53		75.01016

				223.55		74.99391

				223.57		74.96953

				223.59		74.95329

				223.61		74.92485

				223.63		74.90454

				223.66		74.88017

				223.68		74.86798

				223.7		74.83549

				223.72		74.81111

				223.74		74.7908

				223.76		74.76643

				223.78		74.72987

				223.8		74.71769

				223.82		74.69331

				223.84		74.66082

				223.87		74.64051

				223.89		74.62832

				223.91		74.60395

				223.93		74.58364

				223.95		74.56739

				223.97		74.53489

				223.99		74.50646

				224.01		74.47802

				224.03		74.45365

				224.05		74.43334

				224.08		74.41709

				224.1		74.39678

				224.12		74.37647

				224.14		74.34804

				224.16		74.3196

				224.18		74.29117

				224.2		74.27086

				224.22		74.25055

				224.24		74.22618

				224.26		74.2018

				224.28		74.18556

				224.31		74.16118

				224.33		74.13275

				224.35		74.10838

				224.37		74.084

				224.39		74.06369

				224.41		74.03932

				224.43		74.02307

				224.45		74.00682

				224.47		73.99058

				224.49		73.96214

				224.52		73.94996

				224.54		73.91746

				224.56		73.89309

				224.58		73.86059

				224.6		73.84028

				224.62		73.80372

				224.64		73.77935

				224.66		73.75904

				224.68		73.7306

				224.7		73.70623

				224.73		73.68186

				224.75		73.66561

				224.77		73.63718

				224.79		73.62093

				224.81		73.59656

				224.83		73.58031

				224.85		73.55187

				224.87		73.53156

				224.89		73.50719

				224.91		73.47876

				224.93		73.45438

				224.96		73.43407

				224.98		73.40564

				225		73.3772

				225.02		73.35689

				225.04		73.3244

				225.06		73.30409

				225.08		73.28784

				225.1		73.27565

				225.12		73.25128

				225.14		73.23909

				225.17		73.21066

				225.19		73.18629

				225.21		73.14973

				225.23		73.13348

				225.25		73.10505

				225.27		73.08473

				225.29		73.06442

				225.31		73.04005

				225.33		72.99943

				225.35		72.97912

				225.37		72.95475

				225.4		72.92631

				225.42		72.91007

				225.44		72.89382

				225.46		72.86538

				225.48		72.8532

				225.5		72.83289

				225.52		72.79633

				225.54		72.77602

				225.56		72.75977

				225.58		72.73133

				225.61		72.69884

				225.63		72.68665

				225.65		72.65822

				225.67		72.63385

				225.69		72.61353

				225.71		72.59322

				225.73		72.56073

				225.75		72.53229

				225.77		72.50386

				225.79		72.47949

				225.82		72.45105

				225.84		72.43074

				225.86		72.41043

				225.88		72.39418

				225.9		72.35762

				225.92		72.34138

				225.94		72.30888

				225.96		72.28451

				225.98		72.25607

				226		72.24389

				226.02		72.21139

				226.05		72.20327

				226.07		72.16671

				226.09		72.15046

				226.11		72.11796

				226.13		72.10984

				226.15		72.0814

				226.17		72.06109

				226.19		72.03672

				226.21		72.01235

				226.23		71.97579

				226.26		71.94329

				226.28		71.92298

				226.3		71.89455

				226.32		71.87424

				226.34		71.85393

				226.36		71.82549

				226.38		71.80112

				226.4		71.77675

				226.42		71.75644

				226.44		71.728

				226.46		71.70769

				226.49		71.6752

				226.51		71.65082

				226.53		71.61427

				226.55		71.58989

				226.57		71.56146

				226.59		71.53709

				226.61		71.50459

				226.63		71.48834

				226.65		71.46397

				226.67		71.4396

				226.69		71.41116

				226.72		71.38679

				226.74		71.35429

				226.76		71.32992

				226.78		71.30555

				226.8		71.28524

				226.82		71.2568

				226.84		71.24056

				226.86		71.20806

				226.88		71.18369

				226.9		71.16338

				226.92		71.139

				226.95		71.10651

				226.97		71.09432

				226.99		71.06589

				227.01		71.03745

				227.03		71.00902

				227.05		70.98465

				227.07		70.94402

				227.09		70.91965

				227.11		70.89122

				227.13		70.87091

				227.15		70.84654

				227.18		70.83029

				227.2		70.80591

				227.22		70.7856

				227.24		70.75311

				227.26		70.7328

				227.28		70.7003

				227.3		70.67593

				227.32		70.64749

				227.34		70.62718

				227.36		70.59469

				227.38		70.57844

				227.41		70.54594

				227.43		70.51751

				227.45		70.48907

				227.47		70.4647

				227.49		70.42814

				227.51		70.39971

				227.53		70.36721

				227.55		70.3469

				227.57		70.31847

				227.59		70.29816

				227.61		70.26972

				227.64		70.24941

				227.66		70.21285

				227.68		70.1966

				227.7		70.17223

				227.72		70.14786

				227.74		70.11942

				227.76		70.10318

				227.78		70.06256

				227.8		70.03412

				227.82		70.00975

				227.84		69.98131

				227.87		69.95288

				227.89		69.93257

				227.91		69.90414

				227.93		69.88382

				227.95		69.85945

				227.97		69.83914

				227.99		69.81477

				228.01		69.7904

				228.03		69.7579

				228.05		69.7254

				228.07		69.69291

				228.1		69.66041

				228.12		69.63198

				228.14		69.59948

				228.16		69.57511

				228.18		69.54667

				228.2		69.51011

				228.22		69.48168

				228.24		69.46543

				228.26		69.437

				228.28		69.40856

				228.3		69.38825

				228.32		69.36388

				228.35		69.33951

				228.37		69.31107

				228.39		69.29076

				228.41		69.26639

				228.43		69.23796

				228.45		69.20952

				228.47		69.19327

				228.49		69.15671

				228.51		69.13234

				228.53		69.09985

				228.55		69.07141

				228.58		69.03485

				228.6		69.0186

				228.62		68.98611

				228.64		68.96174

				228.66		68.94549

				228.68		68.92111

				228.7		68.88862

				228.72		68.87237

				228.74		68.83987

				228.76		68.80738

				228.78		68.77488

				228.81		68.75051

				228.83		68.72207

				228.85		68.70176

				228.87		68.67333

				228.89		68.64489

				228.91		68.61646

				228.93		68.58396

				228.95		68.55959

				228.97		68.53522

				228.99		68.51085

				229.01		68.48647

				229.03		68.45398

				229.06		68.42148

				229.08		68.38898

				229.1		68.36055

				229.12		68.32399

				229.14		68.30368

				229.16		68.27525

				229.18		68.259

				229.2		68.21838

				229.22		68.19807

				229.24		68.17369

				229.26		68.1412

				229.28		68.1087

				229.31		68.08027

				229.33		68.05589

				229.35		68.0234

				229.37		68.00715

				229.39		67.97059

				229.41		67.95434

				229.43		67.92997

				229.45		67.90154

				229.47		67.86091

				229.49		67.84467

				229.51		67.81623

				229.54		67.77561

				229.56		67.74718

				229.58		67.73093

				229.6		67.70249

				229.62		67.66594

				229.64		67.65375

				229.66		67.62938

				229.68		67.59688

				229.7		67.54814

				229.72		67.52376

				229.74		67.49533

				229.77		67.46283

				229.79		67.43034

				229.81		67.41409

				229.83		67.38971

				229.85		67.35316

				229.87		67.32066

				229.89		67.29223

				229.91		67.26379

				229.93		67.23129

				229.95		67.20692

				229.97		67.17849

				229.99		67.15818

				230.02		67.12974

				230.04		67.09725

				230.06		67.07287

				230.08		67.0485

				230.1		67.016

				230.12		66.97538

				230.14		66.9632

				230.16		66.91851

				230.18		66.89008

				230.2		66.86571

				230.22		66.8454

				230.25		66.80884

				230.27		66.78853

				230.29		66.75603

				230.31		66.7276

				230.33		66.69916

				230.35		66.67073

				230.37		66.64229

				230.39		66.6098

				230.41		66.5773

				230.43		66.55293

				230.45		66.52043

				230.47		66.48794

				230.5		66.47169

				230.52		66.43919

				230.54		66.40263

				230.56		66.38232

				230.58		66.35389

				230.6		66.31733

				230.62		66.29296

				230.64		66.26046

				230.66		66.22796

				230.68		66.19953

				230.7		66.17109

				230.72		66.14266

				230.75		66.11829

				230.77		66.08985

				230.79		66.05736

				230.81		66.02892

				230.83		66.00049

				230.85		65.98018

				230.87		65.94362

				230.89		65.93143

				230.91		65.89894

				230.93		65.87456

				230.95		65.82176

				230.98		65.81363

				231		65.76895

				231.02		65.73645

				231.04		65.70802

				231.06		65.69177

				231.08		65.64709

				231.1		65.61865

				231.12		65.58616

				231.14		65.56178

				231.16		65.52523

				231.18		65.49273

				231.2		65.46836

				231.23		65.43992

				231.25		65.3993

				231.27		65.37899

				231.29		65.35056

				231.31		65.32212

				231.33		65.28556

				231.35		65.26119

				231.37		65.22463

				231.39		65.20026

				231.41		65.17183

				231.43		65.14339

				231.45		65.11089

				231.48		65.07027

				231.5		65.04996

				231.52		65.0134

				231.54		64.98497

				231.56		64.95654

				231.58		64.93623

				231.6		64.90779

				231.62		64.87936

				231.64		64.86717

				231.66		64.83874

				231.68		64.80218

				231.71		64.75343

				231.73		64.70875

				231.75		64.66

				231.77		64.62345

				231.79		64.58689

				231.81		64.55845

				231.83		64.53408

				231.85		64.50158

				231.87		64.46909

				231.89		64.44878

				231.91		64.43253

				231.93		64.40409

				231.96		64.37566

				231.98		64.34723

				232		64.32285

				232.02		64.27817

				232.04		64.25786

				232.06		64.2213

				232.08		64.1888

				232.1		64.15631

				232.12		64.13194

				232.14		64.08319

				232.16		64.05882

				232.19		64.02632

				232.21		63.96945

				232.23		63.91665

				232.25		63.97352

				232.27		63.92477

				232.29		63.93289

				232.31		63.91258

				232.33		63.90852

				232.35		63.80291

				232.37		63.78666

				232.39		63.71354

				232.41		63.69729

				232.44		63.65667

				232.46		63.6323

				232.48		63.58762

				232.5		63.56731

				232.52		63.53887

				232.54		63.51044

				232.56		63.47388

				232.58		63.45357

				232.6		63.41295

				232.62		63.38045

				232.64		63.34796

				232.66		63.31546

				232.69		63.28703

				232.71		63.25859

				232.73		63.21797

				232.75		63.1936

				232.77		63.1611

				232.79		63.12454

				232.81		63.08392

				232.83		63.06767

				232.85		63.01893

				232.87		62.98643

				232.89		62.958

				232.91		62.93363

				232.94		62.89301

				232.96		62.87269

				232.98		62.84426

				233		62.81176

				233.02		62.78333

				233.04		62.75083

				233.06		62.71427

				233.08		62.68584

				233.1		62.65334

				233.12		62.60866

				233.14		62.5721

				233.17		62.54773

				233.19		62.50305

				233.21		62.46649

				233.23		62.44618

				233.25		62.42181

				233.27		62.38931

				233.29		62.36087

				233.31		62.33244

				233.33		62.29994

				233.35		62.26338

				233.37		62.23089

				233.39		62.20245

				233.42		62.16589

				233.44		62.1334

				233.46		62.10903

				233.48		62.06434

				233.5		62.03591

				233.52		62.00341

				233.54		61.96685

				233.56		61.92217

				233.58		61.90592

				233.6		61.86936

				233.62		61.83281

				233.64		61.80437

				233.67		61.78

				233.69		61.73125

				233.71		61.69876

				233.73		61.6622

				233.75		61.63783

				233.77		61.60127

				233.79		61.57689

				233.81		61.54846

				233.83		61.53221

				233.85		61.48753

				233.87		61.45503

				233.89		61.42254

				233.92		61.39004

				233.94		61.34942

				233.96		61.31692

				233.98		61.2763

				234		61.25193

				234.02		61.21131

				234.04		61.17069

				234.06		61.13819

				234.08		61.11382

				234.1		61.07726

				234.12		61.04883

				234.14		61.01227

				234.17		60.98383

				234.19		60.94727

				234.21		60.91072

				234.23		60.87416

				234.25		60.85385

				234.27		60.81323

				234.29		60.78479

				234.31		60.74823

				234.33		60.71574

				234.35		60.67918

				234.37		60.64668

				234.39		60.602

				234.42		60.58169

				234.44		60.54919

				234.46		60.50857

				234.48		60.47607

				234.5		60.4517

				234.52		60.41514

				234.54		60.37858

				234.56		60.34609

				234.58		60.31359

				234.6		60.27297

				234.62		60.2486

				234.64		60.2161

				234.67		60.17954

				234.69		60.13486

				234.71		60.0983

				234.73		60.05768

				234.75		60.02112

				234.77		59.98863

				234.79		59.96019

				234.81		59.9277

				234.83		59.89926

				234.85		59.87083

				234.87		59.83427

				234.89		59.79365

				234.91		59.76521

				234.94		59.72459

				234.96		59.68397

				234.98		59.65554

				235		59.62304

				235.02		59.58648

				235.04		59.55398

				235.06		59.51743

				235.08		59.48899

				235.1		59.45243

				235.12		59.41994

				235.14		59.38744

				235.16		59.35901

				235.19		59.31432

				235.21		59.28183

				235.23		59.24527

				235.25		59.20871

				235.27		59.17621

				235.29		59.13965

				235.31		59.09903

				235.33		59.06247

				235.35		59.02998

				235.37		58.98936

				235.39		58.96092

				235.41		58.92843

				235.43		58.89187

				235.46		58.85125

				235.48		58.82281

				235.5		58.77813

				235.52		58.74157

				235.54		58.70095

				235.56		58.67658

				235.58		58.63596

				235.6		58.60346

				235.62		58.57909

				235.64		58.54659

				235.66		58.51003

				235.68		58.47754

				235.71		58.43692

				235.73		58.39223

				235.75		58.35567

				235.77		58.31912

				235.79		58.28662

				235.81		58.25412

				235.83		58.22975

				235.85		58.19725

				235.87		58.15257

				235.89		58.11601

				235.91		58.07945

				235.93		58.03477

				235.96		58.00227

				235.98		57.9779

				236		57.94947

				236.02		57.9251

				236.04		57.88854

				236.06		57.84385

				236.08		57.80323

				236.1		57.76261

				236.12		57.72199

				236.14		57.68137

				236.16		57.64887

				236.18		57.61638

				236.21		57.58388

				236.23		57.54326

				236.25		57.52701

				236.27		57.52701

				236.29		57.50264

				236.31		57.44171

				236.33		57.40921

				236.35		57.34828

				236.37		57.27923

				236.39		57.21423

				236.41		57.19799

				236.43		57.16143

				236.46		57.13299

				236.48		57.1005

				236.5		57.07612

				236.52		57.04769

				236.54		57.01519

				236.56		56.98676

				236.58		56.94614

				236.6		56.90958

				236.62		56.87708

				236.64		56.82834

				236.66		56.7999

				236.68		56.76741

				236.71		56.72272

				236.73		56.6821

				236.75		56.65773

				236.77		56.61305

				236.79		56.57649

				236.81		56.54399

				236.83		56.5115

				236.85		56.47494

				236.87		56.43025

				236.89		56.38963

				236.91		56.31652

				236.93		56.32058

				236.96		56.28808

				236.98		56.23934

				237		56.21496

				237.02		56.21496

				237.04		56.15403

				237.06		56.10935

				237.08		56.0931

				237.1		56.05654

				237.12		56.02405

				237.14		55.96718

				237.16		55.93062

				237.19		55.89406

				237.21		55.84938

				237.23		55.80876

				237.25		55.77626

				237.27		55.73564

				237.29		55.69096

				237.31		55.65846

				237.33		55.63003

				237.35		55.58941

				237.37		55.55691

				237.39		55.52848

				237.41		55.48785

				237.44		55.44317

				237.46		55.40255

				237.48		55.37005

				237.5		55.32537

				237.52		55.30506

				237.54		55.26444

				237.56		55.23194

				237.58		55.17914

				237.6		55.14258

				237.62		55.09383

				237.64		55.0654

				237.66		55.02072

				237.69		55.00041

				237.71		54.96791

				237.73		54.93541

				237.75		54.89885

				237.77		54.85823

				237.79		54.81355

				237.81		54.77699

				237.83		54.74043

				237.85		54.69575

				237.87		54.65513

				237.89		54.6267

				237.91		54.57795

				237.94		54.54139

				237.96		54.50077

				237.98		54.46421

				238		54.43172

				238.02		54.39922

				238.04		54.34641

				238.06		54.32204

				238.08		54.28954

				238.1		54.24892

				238.12		54.20424

				238.14		54.17987

				238.16		54.13925

				238.19		54.09863

				238.21		54.05801

				238.23		54.03363

				238.25		53.98489

				238.27		53.93614

				238.29		53.89552

				238.31		53.8549

				238.33		53.81428

				238.35		53.78585

				238.37		53.74929

				238.39		53.70867

				238.42		53.66399

				238.44		53.62743

				238.46		53.57868

				238.48		53.54619

				238.5		53.51369

				238.52		53.48119

				238.54		53.43245

				238.56		53.39995

				238.58		53.36339

				238.6		53.32683

				238.62		53.28621

				238.65		53.25372

				238.67		53.20903

				238.69		53.16841

				238.71		53.12779

				238.73		53.09123

				238.75		53.03843

				238.77		53.00593

				238.79		52.96531

				238.81		52.92875

				238.83		52.89219

				238.85		52.8597

				238.87		52.81095

				238.9		52.78252

				238.92		52.75408

				238.94		52.71752

				238.96		52.67284

				238.98		52.63628

				239		52.59566

				239.02		52.53879

				239.04		52.5063

				239.06		52.47786

				239.08		52.4413

				239.1		52.40068

				239.13		52.36819

				239.15		52.32757

				239.17		52.28694

				239.19		52.24226

				239.21		52.19758

				239.23		52.16914

				239.25		52.1204

				239.27		52.07978

				239.29		52.04322

				239.31		52.0026

				239.33		51.96198

				239.35		51.92948

				239.38		51.88074

				239.4		51.8523

				239.42		51.81574

				239.44		51.77512

				239.46		51.73044

				239.48		51.69388

				239.5		51.64514

				239.52		51.60045

				239.54		51.55983

				239.56		51.52328

				239.58		51.48672

				239.61		51.44203

				239.63		51.40954

				239.65		51.37298

				239.67		51.3283

				239.69		51.28768

				239.71		51.25518

				239.73		51.20643

				239.75		51.15769

				239.77		51.12519

				239.79		51.08051

				239.81		51.03177

				239.83		51.00333

				239.86		50.97083

				239.88		50.92615

				239.9		50.89366

				239.92		50.86116

				239.94		50.81648

				239.96		50.77179

				239.98		50.73117

				240		50.69461

				240.02		50.64587

				240.04		50.59306

				240.06		50.5565

				240.09		50.51182

				240.11		50.46714

				240.13		50.42246

				240.15		50.3859

				240.17		50.34121

				240.19		50.30466

				240.21		50.25997

				240.23		50.21935

				240.25		50.18686

				240.27		50.14623

				240.29		50.10155

				240.31		50.06906

				240.34		50.02843

				240.36		49.97969

				240.38		49.94313

				240.4		49.91063

				240.42		49.87001

				240.44		49.83752

				240.46		49.80096

				240.48		49.75628

				240.5		49.71159

				240.52		49.67097

				240.54		49.63035

				240.57		49.57754

				240.59		49.53692

				240.61		49.50037

				240.63		49.45162

				240.65		49.40694

				240.67		49.3785

				240.69		49.32976

				240.71		49.28508

				240.73		49.24852

				240.75		49.20383

				240.77		49.16321

				240.8		49.11853

				240.82		49.08197

				240.84		49.04541

				240.86		49.00479

				240.88		48.96011

				240.9		48.93168

				240.92		48.89106

				240.94		48.83825

				240.96		48.80575

				240.98		48.76919

				241		48.71232

				241.02		48.6717

				241.05		48.63108

				241.07		48.59046

				241.09		48.54578

				241.11		48.50922

				241.13		48.46454

				241.15		48.42392

				241.17		48.3833

				241.19		48.33861

				241.21		48.29393

				241.23		48.25331

				241.25		48.21269

				241.28		48.15988

				241.3		48.11926

				241.32		48.07052

				241.34		48.04615

				241.36		47.9974

				241.38		47.9649

				241.4		47.91616

				241.42		47.88772

				241.44		47.83492

				241.46		47.7943

				241.48		47.74149

				241.51		47.70899

				241.53		47.66025

				241.55		47.61557

				241.57		47.5587

				241.59		47.5262

				241.61		47.47339

				241.63		47.43277

				241.65		47.39215

				241.67		47.37184

				241.69		47.32716

				241.71		47.28654

				241.74		47.24592

				241.76		47.20936

				241.78		47.15249

				241.8		47.11593

				241.82		47.07125

				241.84		47.03469

				241.86		46.98595

				241.88		46.9372

				241.9		46.88439

				241.92		46.84783

				241.94		46.79909

				241.97		46.75847

				241.99		46.71379

				242.01		46.68129

				242.03		46.63661

				242.05		46.59192

				242.07		46.55537

				242.09		46.52693

				242.11		46.47412

				242.13		46.42538

				242.15		46.37663

				242.17		46.34008

				242.2		46.28727

				242.22		46.24259

				242.24		46.20603

				242.26		46.17353

				242.28		46.12479

				242.3		46.07604

				242.32		46.03542

				242.34		45.99074

				242.36		45.94199

				242.38		45.89731

				242.4		45.85669

				242.43		45.81201

				242.45		45.76326

				242.47		45.71046

				242.49		45.66577

				242.51		45.62515

				242.53		45.58453

				242.55		45.53579

				242.57		45.49517

				242.59		45.45048

				242.61		45.40174

				242.63		45.36518

				242.65		45.32862

				242.68		45.288

				242.7		45.24332

				242.72		45.19457

				242.74		45.14583

				242.76		45.10115

				242.78		45.04834

				242.8		45.00772

				242.82		44.95897

				242.84		44.91429

				242.86		44.87367

				242.88		44.83711

				242.91		44.79243

				242.93		44.76806

				242.95		44.72744

				242.97		44.67869

				242.99		44.63401

				243.01		44.58932

				243.03		44.53246

				243.05		44.47965

				243.07		44.44309

				243.09		44.39435

				243.11		44.35372

				243.13		44.30498

				243.16		44.2603

				243.18		44.21155

				243.2		44.15875

				243.22		44.11

				243.24		44.06938

				243.26		44.03282

				243.28		43.99626

				243.3		43.95564

				243.32		43.9069

				243.34		43.8744

				243.36		43.82566

				243.38		43.77285

				243.41		43.72817

				243.43		43.69567

				243.45		43.64286

				243.47		43.59818

				243.49		43.56162

				243.51		43.52913

				243.53		43.48038

				243.55		43.43976

				243.57		43.39914

				243.59		43.36258

				243.61		43.30977

				243.64		43.26915

				243.66		43.22447

				243.68		43.17166

				243.7		43.12698

				243.72		43.07824

				243.74		43.02949

				243.76		42.98481

				243.78		42.93606

				243.8		42.87919

				243.82		42.83451

				243.84		42.78983

				243.87		42.74108

				243.89		42.70453

				243.91		42.66797

				243.93		42.62735

				243.95		42.58673

				243.97		42.5461

				243.99		42.48924

				244.01		42.44861

				244.03		42.39581

				244.05		42.34706

				244.07		42.29832

				244.09		42.25364

				244.12		42.20083

				244.14		42.16021

				244.16		42.11146

				244.18		42.06678

				244.2		42.0221

				244.22		41.98148

				244.24		41.92867

				244.26		41.89211

				244.28		41.84743

				244.3		41.79868

				244.32		41.74994

				244.35		41.70932

				244.37		41.65651

				244.39		41.6037

				244.41		41.55496

				244.43		41.5184

				244.45		41.46153

				244.47		41.42497

				244.49		41.38029

				244.51		41.34373

				244.53		41.29093

				244.55		41.25437

				244.58		41.20156

				244.6		41.16094

				244.62		41.12032

				244.64		41.06751

				244.66		41.02689

				244.68		40.98221

				244.7		40.9294

				244.72		40.88066

				244.74		40.84004

				244.76		40.79129

				244.78		40.75067

				244.8		40.69786

				244.83		40.64912

				244.85		40.61662

				244.87		40.56382

				244.89		40.51507

				244.91		40.47851

				244.93		40.43789

				244.95		40.3729

				244.97		40.33228

				244.99		40.27947

				245.01		40.22666

				245.03		40.17792

				245.06		40.14542

				245.08		40.08449

				245.1		40.04387

				245.12		39.99919

				245.14		39.9545

				245.16		39.89357

				245.18		39.86514

				245.2		39.82046

				245.22		39.76765

				245.24		39.72703

				245.26		39.68235

				245.28		39.62548

				245.31		39.58486

				245.33		39.53205

				245.35		39.48737

				245.37		39.44268

				245.39		39.398

				245.41		39.34113

				245.43		39.31676

				245.45		39.25583

				245.47		39.20708

				245.49		39.1624

				245.51		39.10553

				245.54		39.05273

				245.56		39.00804

				245.58		38.96336

				245.6		38.91868

				245.62		38.87806

				245.64		38.82525

				245.66		38.76838

				245.68		38.72776

				245.7		38.67495

				245.72		38.62621

				245.74		38.58153

				245.77		38.54497

				245.79		38.48404

				245.81		38.44342

				245.83		38.38248

				245.85		38.3378

				245.87		38.28093

				245.89		38.24031

				245.91		38.18344

				245.93		38.13876

				245.95		38.09002

				245.97		38.04127

				246		37.98846

				246.02		37.94378

				246.04		37.8991

				246.06		37.84223

				246.08		37.79348

				246.1		37.75286

				246.12		37.70412

				246.14		37.65131

				246.16		37.61069

				246.18		37.56195

				246.2		37.5132

				246.23		37.45227

				246.25		37.40759

				246.27		37.35884

				246.29		37.31416

				246.31		37.25729

				246.33		37.22073

				246.35		37.17605

				246.37		37.12731

				246.39		37.07856

				246.41		37.03388

				246.43		36.98107

				246.46		36.92826

				246.48		36.88764

				246.5		36.83077

				246.52		36.79422

				246.54		36.74953

				246.56		36.69673

				246.58		36.64392

				246.6		36.59517

				246.62		36.53424

				246.64		36.48144

				246.66		36.44082

				246.69		36.38801

				246.71		36.33926

				246.73		36.29052

				246.75		36.2499

				246.77		36.19709

				246.79		36.14022

				246.81		36.09148

				246.83		36.05492

				246.85		35.99399

				246.87		35.94524

				246.89		35.90056

				246.92		35.85588

				246.94		35.8112

				246.96		35.75839

				246.98		35.72183

				247		35.66496

				247.02		35.61215

				247.04		35.55122

				247.06		35.5106

				247.08		35.45373

				247.1		35.41311

				247.12		35.36843

				247.15		35.32781

				247.17		35.275

				247.19		35.22626

				247.21		35.16533

				247.23		35.11252

				247.25		35.06784

				247.27		35.01909

				247.29		34.97441

				247.31		34.92566

				247.33		34.8688

				247.35		34.82005

				247.38		34.75912

				247.4		34.69819

				247.42		34.65351

				247.44		34.60882

				247.46		34.55195

				247.48		34.50321

				247.5		34.46259

				247.52		34.40572

				247.54		34.34885

				247.56		34.30417

				247.58		34.26355

				247.61		34.2148

				247.63		34.162

				247.65		34.12137

				247.67		34.08075

				247.69		34.02388

				247.71		33.97514

				247.73		33.93452

				247.75		33.88171

				247.77		33.82891

				247.79		33.76797

				247.82		33.71517

				247.84		33.66236

				247.86		33.60955

				247.88		33.56081

				247.9		33.51613

				247.92		33.46738

				247.94		33.41051

				247.96		33.35364

				247.98		33.30084

				248		33.25615

				248.02		33.20741

				248.05		33.1546

				248.07		33.10992

				248.09		33.06524

				248.11		33.01649

				248.13		32.96369

				248.15		32.91494

				248.17		32.8662

				248.19		32.80933

				248.21		32.75652

				248.23		32.70371

				248.25		32.65903

				248.28		32.60622

				248.3		32.55748

				248.32		32.50061

				248.34		32.45186

				248.36		32.40312

				248.38		32.35437

				248.4		32.30157

				248.42		32.26095

				248.44		32.20814

				248.46		32.14315

				248.49		32.08628

				248.51		32.03753

				248.53		31.98066

				248.55		31.93192

				248.57		31.88724

				248.59		31.84255

				248.61		31.78975

				248.63		31.72475

				248.65		31.67601

				248.67		31.63133

				248.69		31.57446

				248.72		31.52977

				248.74		31.47697

				248.76		31.42416

				248.78		31.36729

				248.8		31.30636

				248.82		31.24949

				248.84		31.21293

				248.86		31.16013

				248.88		31.10732

				248.9		31.06264

				248.93		31.01795

				248.95		30.96109

				248.97		30.90422

				248.99		30.85547

				249.01		30.81079

				249.03		30.74986

				249.05		30.69299

				249.07		30.64424

				249.09		30.5955

				249.11		30.53457

				249.13		30.48176

				249.16		30.42895

				249.18		30.38427

				249.2		30.33146

				249.22		30.27866

				249.24		30.22991

				249.26		30.18523

				249.28		30.13242

				249.3		30.06337

				249.32		30.01869

				249.34		29.96588

				249.37		29.90901

				249.39		29.8562

				249.41		29.80746

				249.43		29.75465

				249.45		29.70997

				249.47		29.64904

				249.49		29.59623

				249.51		29.54749

				249.53		29.49062

				249.55		29.43375

				249.58		29.39719

				249.6		29.34032

				249.62		29.29158

				249.64		29.23471

				249.66		29.18596

				249.68		29.12097

				249.7		29.07222

				249.72		29.00317

				249.74		28.95849

				249.76		28.90568

				249.78		28.85287

				249.81		28.80413

				249.83		28.76351

				249.85		28.7107

				249.87		28.65789

				249.89		28.60509

				249.91		28.54822

				249.93		28.49947

				249.95		28.4426

				249.97		28.3898

				249.99		28.33293

				250.02		28.272

				250.04		28.22325

				250.06		28.17451

				250.08		28.11358

				250.1		28.06483

				250.12		28.01609

				250.14		27.95515

				250.16		27.89016

				250.18		27.84548

				250.2		27.78861

				250.22		27.7358

				250.25		27.683

				250.27		27.64238

				250.29		27.58551

				250.31		27.53676

				250.33		27.47989

				250.35		27.43115

				250.37		27.37428

				250.39		27.31741

				250.41		27.26054

				250.43		27.21586

				250.46		27.15087

				250.48		27.11024

				250.5		27.05744

				250.52		27.00869

				250.54		26.95182

				250.56		26.89495

				250.58		26.8259

				250.6		26.78528

				250.62		26.72841

				250.64		26.67967

				250.66		26.62686

				250.69		26.58218

				250.71		26.51718

				250.73		26.45625

				250.75		26.40751

				250.77		26.3547

				250.79		26.29783

				250.81		26.24909

				250.83		26.20034

				250.85		26.14753

				250.87		26.09067

				250.89		26.0338

				250.92		25.9688

				250.94		25.91193

				250.96		25.85913

				250.98		25.81038

				251		25.76164

				251.02		25.71289

				251.04		25.65196

				251.06		25.59103

				251.08		25.53416

				251.1		25.46917

				251.13		25.42042

				251.15		25.36762

				251.17		25.31481

				251.19		25.262

				251.21		25.2092

				251.23		25.14827

				251.25		25.0914

				251.27		25.03859

				251.29		24.98172

				251.31		24.9411

				251.33		24.88829

				251.36		24.83549

				251.38		24.78268

				251.4		24.72987

				251.42		24.65676

				251.44		24.60801

				251.46		24.5552

				251.48		24.49833

				251.5		24.43334

				251.52		24.38866

				251.54		24.32773

				251.57		24.2668

				251.59		24.21399

				251.61		24.16931

				251.63		24.10838

				251.65		24.05557

				251.67		24.00276

				251.69		23.94589

				251.71		23.88902

				251.73		23.83216

				251.75		23.77529

				251.77		23.7306

				251.8		23.6778

				251.82		23.62093

				251.84		23.57218

				251.86		23.51531

				251.88		23.45845

				251.9		23.40158

				251.92		23.33658

				251.94		23.28378

				251.96		23.23097

				251.98		23.17004

				252.01		23.10911

				252.03		23.06849

				252.05		23.00756

				252.07		22.95881

				252.09		22.906

				252.11		22.86538

				252.13		22.79633

				252.15		22.74758

				252.17		22.68259

				252.19		22.63791

				252.22		22.56885

				252.24		22.51605

				252.26		22.45511

				252.28		22.40231

				252.3		22.34138

				252.32		22.28857

				252.34		22.23576

				252.36		22.18702

				252.38		22.13421

				252.4		22.07734

				252.42		22.01235

				252.45		21.96767

				252.47		21.90673

				252.49		21.85393

				252.51		21.79706

				252.53		21.75644

				252.55		21.69145

				252.57		21.63051

				252.59		21.57365

				252.61		21.52084

				252.63		21.45991

				252.66		21.39898

				252.68		21.35429

				252.7		21.29742

				252.72		21.24056

				252.74		21.18369

				252.76		21.12682

				252.78		21.06995

				252.8		21.01714

				252.82		20.95215

				252.84		20.9034

				252.86		20.8506

				252.89		20.78967

				252.91		20.72874

				252.93		20.68405

				252.95		20.62312

				252.97		20.56219

				252.99		20.51345

				253.01		20.4647

				253.03		20.40783

				253.05		20.35502

				253.07		20.29409

				253.1		20.24535

				253.12		20.18442

				253.14		20.12349

				253.16		20.06256

				253.18		20.00975

				253.2		19.94069

				253.22		19.88382

				253.24		19.81883

				253.26		19.76602

				253.28		19.71322

				253.31		19.66041

				253.33		19.59542

				253.35		19.55074

				253.37		19.49793

				253.39		19.44106

				253.41		19.38013

				253.43		19.32732

				253.45		19.27451

				253.47		19.20952

				253.49		19.14859

				253.51		19.09985

				253.54		19.03485

				253.56		18.98205

				253.58		18.92518

				253.6		18.86831

				253.62		18.79925

				253.64		18.75051

				253.66		18.68145

				253.68		18.62865

				253.7		18.56771

				253.72		18.51897

				253.75		18.4621

				253.77		18.41742

				253.79		18.34836

				253.81		18.29962

				253.83		18.24275

				253.85		18.18994

				253.87		18.13714

				253.89		18.08433

				253.91		18.01934

				253.93		17.97059

				253.96		17.91372

				253.98		17.84467

				254		17.7878

				254.02		17.73905

				254.04		17.67406

				254.06		17.61313

				254.08		17.55626

				254.1		17.50345

				254.12		17.44658

				254.14		17.38971

				254.16		17.32878

				254.19		17.27191

				254.21		17.21098

				254.23		17.15411

				254.25		17.08912

				254.27		17.03225

				254.29		16.97132

				254.31		16.91445

				254.33		16.84946

				254.35		16.80478

				254.37		16.74385

				254.4		16.69104

				254.42		16.63011

				254.44		16.57324

				254.46		16.50825

				254.48		16.4595

				254.5		16.39451

				254.52		16.34983

				254.54		16.28889

				254.56		16.23609

				254.58		16.17109

				254.61		16.12235

				254.63		16.05329

				254.65		16.00049

				254.67		15.93956

				254.69		15.88269

				254.71		15.82988

				254.73		15.78114

				254.75		15.71614

				254.77		15.67146

				254.79		15.60647

				254.82		15.5496

				254.84		15.48867

				254.86		15.43586

				254.88		15.37493

				254.9		15.32618

				254.92		15.26525

				254.94		15.21651

				254.96		15.14745

				254.98		15.08246

				255		15.02559

				255.02		14.96872

				255.05		14.90373

				255.07		14.85092

				255.09		14.79405

				255.11		14.73312

				255.13		14.68032

				255.15		14.62345

				255.17		14.56252

				255.19		14.51377

				255.21		14.44472

				255.23		14.37972

				255.26		14.33098

				255.28		14.27817

				255.3		14.2213

				255.32		14.17256

				255.34		14.12381

				255.36		14.06288

				255.38		14.01007

				255.4		13.9532

				255.42		13.90446

				255.44		13.83134

				255.46		13.7826

				255.49		13.72573

				255.51		13.6648

				255.53		13.59981

				255.55		13.55512

				255.57		13.49419

				255.59		13.42514

				255.61		13.37233

				255.63		13.3114

				255.65		13.25453

				255.67		13.18954

				255.7		13.14485

				255.72		13.08798

				255.74		13.03112

				255.76		12.97018

				255.78		12.9255

				255.8		12.86457

				255.82		12.79958

				255.84		12.74677

				255.86		12.69396

				255.88		12.61678

				255.9		12.56804

				255.93		12.50711

				255.95		12.45024

				255.97		12.39743

				255.99		12.34869

				256.01		12.28369

				256.03		12.23089

				256.05		12.17808

				256.07		12.11309

				256.09		12.05622

				256.11		12.00341

				256.13		11.95061

				256.16		11.89374

				256.18		11.83281

				256.2		11.78

				256.22		11.72719

				256.24		11.67032

				256.26		11.61752

				256.28		11.56471

				256.3		11.50784

				256.32		11.45097

				256.34		11.38598

				256.37		11.32911

				256.39		11.2763

				256.41		11.21943

				256.43		11.15038

				256.45		11.10163

				256.47		11.03664

				256.49		10.97165

				256.51		10.90665

				256.53		10.85791

				256.55		10.79698

				256.57		10.74417

				256.6		10.67918

				256.62		10.63043

				256.64		10.58169

				256.66		10.52482

				256.68		10.45983

				256.7		10.40702

				256.72		10.34203

				256.74		10.28516

				256.76		10.22016

				256.78		10.1633

				256.8		10.11455

				256.83		10.06174

				256.85		10.00081

				256.87		9.952068

				256.89		9.907385

				256.91		9.846454

				256.93		9.785523

				256.95		9.728654

				256.97		9.675847

				256.99		9.614916

				257.01		9.553985

				257.04		9.509302

				257.06		9.464619

				257.08		9.403688

				257.1		9.342757

				257.12		9.294013

				257.14		9.229019

				257.16		9.168088

				257.18		9.107157

				257.2		9.058413

				257.22		8.997482

				257.24		8.944675

				257.27		8.879682

				257.29		8.830937

				257.31		8.77813

				257.33		8.725323

				257.35		8.664392

				257.37		8.603461

				257.39		8.558778

				257.41		8.493785

				257.43		8.436916

				257.45		8.384109

				257.47		8.335364

				257.5		8.266309

				257.52		8.20944

				257.54		8.156633

				257.56		8.103826

				257.58		8.05102

				257.6		7.990089

				257.62		7.937282

				257.64		7.880413

				257.66		7.819482

				257.68		7.762613

				257.71		7.713868

				257.73		7.656999

				257.75		7.608254

				257.77		7.543261

				257.79		7.486392

				257.81		7.441709

				257.83		7.38484

				257.85		7.307661

				257.87		7.262978

				257.89		7.210171

				257.91		7.14924

				257.94		7.088309

				257.96		7.055813

				257.98		7.007068

				258		6.958323

				258.02		6.901454

				258.04		6.852709

				258.06		6.791778

				258.08		6.734909

				258.1		6.67804

				258.12		6.629296

				258.14		6.580551

				258.17		6.531806

				258.19		6.470875

				258.21		6.414006

				258.23		6.369323

				258.25		6.312454

				258.27		6.243399

				258.29		6.206841

				258.31		6.162158

				258.33		6.101227

				258.35		6.052482

				258.38		6.007799

				258.4		5.954992

				258.42		5.902185

				258.44		5.841254

				258.46		5.788447

				258.48		5.743765

				258.5		5.686896

				258.52		5.630027

				258.54		5.589406

				258.56		5.532537

				258.58		5.483792

				258.61		5.426923

				258.63		5.378179

				258.65		5.32131

				258.67		5.276627

				258.69		5.207572

				258.71		5.166951

				258.73		5.114144

				258.75		5.065399

				258.77		5.004468

				258.79		4.96791

				258.81		4.915103

				258.84		4.866358

				258.86		4.813551

				258.88		4.776992

				258.9		4.724186

				258.92		4.671379

				258.94		4.622634

				258.96		4.569827

				258.98		4.521082

				259		4.468275

				259.02		4.41953

				259.05		4.366724

				259.07		4.334227

				259.09		4.285482

				259.11		4.236737

				259.13		4.192055

				259.15		4.151434

				259.17		4.094565

				259.19		4.04582

				259.21		3.997075

				259.23		3.960517

				259.25		3.903648

				259.28		3.854903

				259.3		3.814282

				259.32		3.769599

				259.34		3.712731

				259.36		3.668048

				259.38		3.631489

				259.4		3.586806

				259.42		3.542124

				259.44		3.505565

				259.46		3.460882

				259.48		3.4162

				259.51		3.375579

				259.53		3.330896

				259.55		3.286213

				259.57		3.257779

				259.59		3.22122

				259.61		3.1806

				259.63		3.148103

				259.65		3.115606

				259.67		3.074986

				259.69		3.030303

				259.71		2.997806

				259.74		2.977496

				259.76		2.932813

				259.78		2.908441

				259.8		2.884069

				259.82		2.84751

				259.84		2.806889

				259.86		2.786579

				259.88		2.758144

				259.9		2.725648

				259.92		2.7094

				259.94		2.680965

				259.97		2.648469

				259.99		2.624096

				260.01		2.603786

				260.03		2.587538

				260.05		2.555041

				260.07		2.538793

				260.09		2.51442

				260.11		2.49411

				260.13		2.465676

				260.15		2.461613

				260.17		2.449427

				260.2		2.437241

				260.22		2.416931

				260.24		2.408807

				260.26		2.388496

				260.28		2.380372

				260.3		2.360062

				260.32		2.356

				260.34		2.343813

				260.36		2.339751

				260.38		2.323503

				260.4		2.319441

				260.43		2.307255

				260.45		2.299131

				260.47		2.286945

				260.49		2.274758

				260.51		2.266634

				260.53		2.266634

				260.55		2.254448

				260.57		2.25851

				260.59		2.254448

				260.61		2.250386

				260.63		2.242262

				260.66		2.234138

				260.68		2.221951

				260.7		2.213827

				260.72		2.209765

				260.74		2.197579

				260.76		2.197579

				260.78		2.193517

				260.8		2.185393

				260.82		2.185393

				260.84		2.185393

				260.86		2.181331

				260.89		2.181331

				260.91		2.173207

				260.93		2.169145

				260.95		2.169145

				260.97		2.169145

				260.99		2.165082

				261.01		2.156958

				261.03		2.152896

				261.05		2.152896

				261.07		2.152896

				261.09		2.148834

				261.12		2.144772

				261.14		2.144772

				261.16		2.14071

				261.18		2.136648

				261.2		2.128524

				261.22		2.128524

				261.24		2.124462

				261.26		2.1204

				261.28		2.1204

				261.3		2.116338

				261.32		2.116338

				261.34		2.112276

				261.37		2.108214

				261.39		2.108214

				261.41		2.108214

				261.43		2.108214

				261.45		2.104151

				261.47		2.100089

				261.49		2.100089

				261.51		2.096027

				261.53		2.096027

				261.55		2.091965

				261.57		2.091965

				261.6		2.091965

				261.62		2.091965

				261.64		2.091965

				261.66		2.091965

				261.68		2.091965

				261.7		2.087903

				261.72		2.087903

				261.74		2.083841

				261.76		2.083841

				261.78		2.083841

				261.8		2.083841

				261.83		2.079779

				261.85		2.079779

				261.87		2.079779

				261.89		2.079779

				261.91		2.079779

				261.93		2.079779

				261.95		2.079779

				261.97		2.075717

				261.99		2.075717

				262.01		2.075717

				262.03		2.075717

				262.06		2.075717

				262.08		2.071655

				262.1		2.071655

				262.12		2.071655

				262.14		2.067593

				262.16		2.067593

				262.18		2.067593

				262.2		2.067593

				262.22		2.063531

				262.24		2.063531

				262.26		2.063531

				262.28		2.063531

				262.31		2.063531

				262.33		2.059469

				262.35		2.059469

				262.37		2.059469

				262.39		2.059469

				262.41		2.059469

				262.43		2.055407

				262.45		2.055407

				262.47		2.055407

				262.49		2.055407

				262.51		2.055407

				262.54		2.051345

				262.56		2.051345

				262.58		2.051345

				262.6		2.051345

				262.62		2.051345

				262.64		2.051345

				262.66		2.047282

				262.68		2.047282

				262.7		2.047282

				262.72		2.04322

				262.74		2.04322

				262.76		2.04322

				262.79		2.04322

				262.81		2.04322

				262.83		2.039158

				262.85		2.039158

				262.87		2.039158

				262.89		2.039158

				262.91		2.035096

				262.93		2.035096

				262.95		2.035096

				262.97		2.031034

				262.99		2.031034

				263.01		2.026972

				263.04		2.026972

				263.06		2.026972

				263.08		2.026972

				263.1		2.026972

				263.12		2.02291

				263.14		2.02291

				263.16		2.02291

				263.18		2.018848

				263.2		2.018848

				263.22		2.018848

				263.24		2.018848

				263.27		2.018848

				263.29		2.018848

				263.31		2.018848

				263.33		2.018848

				263.35		2.018848

				263.37		2.014786

				263.39		2.014786

				263.41		2.014786

				263.43		2.014786

				263.45		2.014786

				263.47		2.014786

				263.49		2.014786

				263.52		2.010724

				263.54		2.014786

				263.56		2.010724

				263.58		2.010724

				263.6		2.010724

				263.62		2.010724

				263.64		2.010724

				263.66		2.010724

				263.68		2.010724

				263.7		2.010724

				263.72		2.006662

				263.75		2.006662

				263.77		2.006662

				263.79		2.006662

				263.81		2.006662

				263.83		2.006662

				263.85		2.006662

				263.87		2.006662

				263.89		2.006662

				263.91		2.006662

				263.93		2.0026

				263.95		2.0026

				263.97		2.0026

				264		2.0026

				264.02		2.0026

				264.04		2.0026

				264.06		1.998538

				264.08		1.998538

				264.1		1.998538

				264.12		1.998538

				264.14		1.998538

				264.16		1.998538

				264.18		1.998538

				264.2		1.998538

				264.23		1.998538

				264.25		1.994476

				264.27		1.994476

				264.29		1.994476

				264.31		1.994476

				264.33		1.994476

				264.35		1.994476

				264.37		1.994476

				264.39		1.990414

				264.41		1.990414

				264.43		1.990414

				264.45		1.990414

				264.48		1.990414

				264.5		1.990414

				264.52		1.990414

				264.54		1.990414

				264.56		1.986351

				264.58		1.986351

				264.6		1.986351

				264.62		1.986351

				264.64		1.986351

				264.66		1.986351

				264.68		1.986351

				264.7		1.986351

				264.73		1.986351

				264.75		1.986351

				264.77		1.986351

				264.79		1.982289

				264.81		1.982289

				264.83		1.982289

				264.85		1.982289

				264.87		1.982289

				264.89		1.982289

				264.91		1.982289

				264.93		1.982289

				264.96		1.978227

				264.98		1.978227

				265		1.978227

				265.02		1.978227

				265.04		1.978227

				265.06		1.974165

				265.08		1.974165

				265.1		1.974165

				265.12		1.974165

				265.14		1.974165

				265.16		1.974165

				265.18		1.974165

				265.21		1.970103

				265.23		1.970103

				265.25		1.970103

				265.27		1.970103

				265.29		1.970103

				265.31		1.966041

				265.33		1.966041

				265.35		1.966041

				265.37		1.966041

				265.39		1.966041

				265.41		1.961979

				265.43		1.961979

				265.46		1.961979

				265.48		1.961979

				265.5		1.961979

				265.52		1.957917

				265.54		1.957917

				265.56		1.957917

				265.58		1.957917

				265.6		1.957917

				265.62		1.953855

				265.64		1.953855

				265.66		1.953855

				265.68		1.953855

				265.71		1.953855

				265.73		1.953855

				265.75		1.953855

				265.77		1.949793

				265.79		1.949793

				265.81		1.949793

				265.83		1.945731

				265.85		1.945731

				265.87		1.945731

				265.89		1.945731

				265.91		1.945731

				265.94		1.945731

				265.96		1.945731

				265.98		1.941669

				266		1.941669

				266.02		1.941669

				266.04		1.941669

				266.06		1.941669

				266.08		1.941669

				266.1		1.941669

				266.12		1.941669

				266.14		1.937607

				266.16		1.937607

				266.19		1.937607

				266.21		1.937607

				266.23		1.937607

				266.25		1.937607

				266.27		1.933545

				266.29		1.933545

				266.31		1.933545

				266.33		1.933545

				266.35		1.933545

				266.37		1.933545

				266.39		1.933545

				266.42		1.929482

				266.44		1.929482

				266.46		1.929482

				266.48		1.929482

				266.5		1.929482

				266.52		1.929482

				266.54		1.929482

				266.56		1.929482

				266.58		1.92542

				266.6		1.92542

				266.62		1.92542

				266.64		1.92542

				266.67		1.92542

				266.69		1.92542

				266.71		1.921358

				266.73		1.921358

				266.75		1.921358

				266.77		1.921358

				266.79		1.921358

				266.81		1.921358

				266.83		1.921358

				266.85		1.917296

				266.87		1.917296

				266.9		1.917296

				266.92		1.917296

				266.94		1.917296

				266.96		1.917296

				266.98		1.917296

				267		1.917296

				267.02		1.913234

				267.04		1.913234

				267.06		1.913234

				267.08		1.913234

				267.1		1.913234

				267.12		1.913234

				267.15		1.909172

				267.17		1.909172

				267.19		1.909172

				267.21		1.909172

				267.23		1.909172

				267.25		1.909172

				267.27		1.909172

				267.29		1.909172

				267.31		1.909172

				267.33		1.90511

				267.35		1.90511

				267.37		1.90511

				267.39		1.90511

				267.42		1.90511

				267.44		1.90511

				267.46		1.90511

				267.48		1.90511

				267.5		1.90511

				267.52		1.90511

				267.54		1.901048

				267.56		1.901048

				267.58		1.901048

				267.6		1.901048

				267.62		1.901048

				267.64		1.901048

				267.67		1.896986

				267.69		1.896986

				267.71		1.896986

				267.73		1.896986

				267.75		1.896986

				267.77		1.896986

				267.79		1.892924

				267.81		1.892924

				267.83		1.892924

				267.85		1.892924

				267.87		1.892924

				267.89		1.892924

				267.91		1.892924

				267.94		1.892924

				267.96		1.888862

				267.98		1.888862

				268		1.888862

				268.02		1.888862

				268.04		1.888862

				268.06		1.888862

				268.08		1.888862

				268.1		1.888862

				268.12		1.888862

				268.14		1.8848

				268.16		1.8848

				268.18		1.8848

				268.21		1.8848

				268.23		1.8848

				268.25		1.8848

				268.27		1.8848

				268.29		1.8848

				268.31		1.8848

				268.33		1.8848

				268.35		1.8848

				268.37		1.880738

				268.39		1.880738

				268.41		1.880738

				268.43		1.880738

				268.45		1.880738

				268.47		1.880738

				268.5		1.880738

				268.52		1.880738

				268.54		1.880738

				268.56		1.880738

				268.58		1.880738

				268.6		1.876676

				268.62		1.876676

				268.64		1.876676

				268.66		1.876676

				268.68		1.876676

				268.7		1.876676

				268.72		1.876676

				268.74		1.876676

				268.77		1.876676

				268.79		1.876676

				268.81		1.876676

				268.83		1.876676

				268.85		1.872614

				268.87		1.872614

				268.89		1.872614

				268.91		1.872614

				268.93		1.872614

				268.95		1.872614

				268.97		1.872614

				268.99		1.872614

				269.01		1.872614

				269.04		1.868551

				269.06		1.868551

				269.08		1.868551

				269.1		1.868551

				269.12		1.868551

				269.14		1.868551

				269.16		1.868551

				269.18		1.868551

				269.2		1.868551

				269.22		1.864489

				269.24		1.864489

				269.26		1.864489

				269.28		1.864489

				269.31		1.864489

				269.33		1.864489

				269.35		1.864489

				269.37		1.864489

				269.39		1.864489

				269.41		1.860427

				269.43		1.860427

				269.45		1.860427

				269.47		1.860427

				269.49		1.860427

				269.51		1.860427

				269.53		1.860427

				269.55		1.860427

				269.58		1.856365

				269.6		1.856365

				269.62		1.856365

				269.64		1.856365

				269.66		1.856365

				269.68		1.856365

				269.7		1.856365

				269.72		1.856365

				269.74		1.856365

				269.76		1.856365

				269.78		1.856365

				269.8		1.856365

				269.82		1.856365

				269.85		1.852303

				269.87		1.852303

				269.89		1.852303

				269.91		1.852303

				269.93		1.852303

				269.95		1.848241

				269.97		1.848241

				269.99		1.848241

				270.01		1.848241

				270.03		1.844179

				270.05		1.844179

				270.07		1.844179

				270.09		1.844179

				270.12		1.840117

				270.14		1.840117

				270.16		1.840117

				270.18		1.840117

				270.2		1.840117

				270.22		1.840117

				270.24		1.836055

				270.26		1.836055

				270.28		1.836055

				270.3		1.836055

				270.32		1.836055

				270.34		1.836055

				270.36		1.836055

				270.39		1.836055

				270.41		1.831993

				270.43		1.831993

				270.45		1.831993

				270.47		1.831993

				270.49		1.831993

				270.51		1.831993

				270.53		1.831993

				270.55		1.831993

				270.57		1.831993

				270.59		1.827931

				270.61		1.827931

				270.63		1.827931

				270.66		1.827931

				270.68		1.827931

				270.7		1.827931

				270.72		1.823869

				270.74		1.823869

				270.76		1.823869

				270.78		1.823869

				270.8		1.823869

				270.82		1.823869

				270.84		1.823869

				270.86		1.823869

				270.88		1.823869

				270.9		1.819807

				270.93		1.819807

				270.95		1.819807

				270.97		1.819807

				270.99		1.819807

				271.01		1.819807

				271.03		1.819807

				271.05		1.819807

				271.07		1.815745

				271.09		1.815745

				271.11		1.815745

				271.13		1.815745

				271.15		1.815745

				271.18		1.815745

				271.2		1.815745

				271.22		1.815745

				271.24		1.811683

				271.26		1.811683

				271.28		1.811683

				271.3		1.811683

				271.32		1.811683

				271.34		1.811683

				271.36		1.811683

				271.38		1.811683

				271.4		1.80762

				271.42		1.80762

				271.45		1.80762

				271.47		1.80762

				271.49		1.80762

				271.51		1.80762

				271.53		1.80762

				271.55		1.80762

				271.57		1.803558

				271.59		1.803558

				271.61		1.803558

				271.63		1.803558

				271.65		1.803558

				271.67		1.803558

				271.7		1.803558

				271.72		1.803558

				271.74		1.803558

				271.76		1.803558

				271.78		1.803558

				271.8		1.803558

				271.82		1.803558

				271.84		1.799496

				271.86		1.799496

				271.88		1.799496

				271.9		1.799496

				271.93		1.799496

				271.95		1.799496

				271.97		1.795434

				271.99		1.795434

				272.01		1.795434

				272.03		1.795434

				272.05		1.795434

				272.07		1.795434

				272.09		1.791372

				272.11		1.791372

				272.13		1.791372

				272.15		1.791372

				272.18		1.791372

				272.2		1.791372

				272.22		1.791372

				272.24		1.791372

				272.26		1.791372

				272.28		1.791372

				272.3		1.791372

				272.32		1.791372

				272.34		1.791372

				272.36		1.78731

				272.38		1.791372

				272.4		1.78731

				272.43		1.78731

				272.45		1.78731

				272.47		1.78731

				272.49		1.78731

				272.51		1.78731

				272.53		1.78731

				272.55		1.78731

				272.57		1.78731

				272.59		1.78731

				272.61		1.783248

				272.63		1.783248

				272.65		1.783248

				272.68		1.783248

				272.7		1.783248

				272.72		1.783248

				272.74		1.783248

				272.76		1.783248

				272.78		1.783248

				272.8		1.779186

				272.82		1.779186

				272.84		1.779186

				272.86		1.779186

				272.88		1.779186

				272.91		1.779186

				272.93		1.779186

				272.95		1.779186

				272.97		1.779186

				272.99		1.775124

				273.01		1.775124

				273.03		1.775124

				273.05		1.775124

				273.07		1.775124

				273.09		1.775124

				273.11		1.775124

				273.13		1.775124

				273.16		1.771062

				273.18		1.771062

				273.2		1.771062

				273.22		1.771062

				273.24		1.771062

				273.26		1.771062

				273.28		1.771062

				273.3		1.767

				273.32		1.767

				273.34		1.767

				273.36		1.767

				273.39		1.767

				273.41		1.767

				273.43		1.767

				273.45		1.767

				273.47		1.767

				273.49		1.767

				273.51		1.767

				273.53		1.767

				273.55		1.762938

				273.57		1.762938

				273.59		1.762938

				273.61		1.762938

				273.64		1.762938

				273.66		1.762938

				273.68		1.762938

				273.7		1.762938

				273.72		1.762938

				273.74		1.762938

				273.76		1.762938

				273.78		1.758876

				273.8		1.758876

				273.82		1.758876

				273.84		1.758876

				273.87		1.758876

				273.89		1.758876

				273.91		1.758876

				273.93		1.758876

				273.95		1.758876

				273.97		1.758876

				273.99		1.758876

				274.01		1.758876

				274.03		1.758876

				274.05		1.754814

				274.07		1.754814

				274.1		1.754814

				274.12		1.754814

				274.14		1.754814

				274.16		1.754814

				274.18		1.754814

				274.2		1.750751

				274.22		1.750751

				274.24		1.750751

				274.26		1.750751

				274.28		1.750751

				274.3		1.750751

				274.33		1.750751

				274.35		1.750751

				274.37		1.746689

				274.39		1.746689

				274.41		1.746689

				274.43		1.746689

				274.45		1.746689

				274.47		1.746689

				274.49		1.746689

				274.51		1.742627

				274.53		1.742627

				274.56		1.742627

				274.58		1.742627

				274.6		1.742627

				274.62		1.742627

				274.64		1.742627

				274.66		1.742627

				274.68		1.742627

				274.7		1.738565

				274.72		1.738565

				274.74		1.738565

				274.76		1.738565

				274.78		1.738565

				274.81		1.738565

				274.83		1.738565

				274.85		1.738565

				274.87		1.738565

				274.89		1.734503

				274.91		1.734503

				274.93		1.734503

				274.95		1.734503

				274.97		1.734503

				274.99		1.734503

				275.01		1.734503

				275.04		1.734503

				275.06		1.734503

				275.08		1.734503

				275.1		1.730441

				275.12		1.730441

				275.14		1.730441

				275.16		1.730441

				275.18		1.730441

				275.2		1.730441

				275.22		1.730441

				275.24		1.730441

				275.27		1.730441

				275.29		1.726379

				275.31		1.726379

				275.33		1.726379

				275.35		1.726379

				275.37		1.726379

				275.39		1.726379

				275.41		1.726379

				275.43		1.726379

				275.45		1.722317

				275.47		1.722317

				275.5		1.722317

				275.52		1.722317

				275.54		1.722317

				275.56		1.722317

				275.58		1.722317

				275.6		1.722317

				275.62		1.722317

				275.64		1.722317

				275.66		1.722317

				275.68		1.722317

				275.7		1.722317

				275.73		1.722317

				275.75		1.722317

				275.77		1.718255

				275.79		1.718255

				275.81		1.718255

				275.83		1.718255

				275.85		1.718255

				275.87		1.718255

				275.89		1.718255

				275.91		1.714193

				275.94		1.714193

				275.96		1.714193

				275.98		1.714193

				276		1.714193

				276.02		1.714193

				276.04		1.714193

				276.06		1.714193

				276.08		1.714193

				276.1		1.714193

				276.12		1.710131

				276.14		1.714193

				276.17		1.710131

				276.19		1.710131

				276.21		1.710131

				276.23		1.710131

				276.25		1.710131

				276.27		1.710131

				276.29		1.710131

				276.31		1.710131

				276.33		1.710131

				276.35		1.710131

				276.37		1.710131

				276.4		1.710131

				276.42		1.710131

				276.44		1.710131

				276.46		1.710131

				276.48		1.710131

				276.5		1.710131

				276.52		1.710131

				276.54		1.710131

				276.56		1.706069

				276.58		1.706069

				276.6		1.706069

				276.63		1.706069

				276.65		1.706069

				276.67		1.706069

				276.69		1.706069

				276.71		1.706069

				276.73		1.706069

				276.75		1.706069

				276.77		1.706069

				276.79		1.706069

				276.81		1.706069

				276.83		1.706069

				276.86		1.706069

				276.88		1.702007

				276.9		1.702007

				276.92		1.702007

				276.94		1.702007

				276.96		1.702007

				276.98		1.706069

				277		1.702007

				277.02		1.702007

				277.04		1.702007

				277.06		1.702007

				277.09		1.702007

				277.11		1.702007

				277.13		1.702007

				277.15		1.702007

				277.17		1.702007

				277.19		1.702007

				277.21		1.702007

				277.23		1.702007

				277.25		1.702007

				277.27		1.702007

				277.3		1.702007

				277.32		1.702007

				277.34		1.702007

				277.36		1.702007

				277.38		1.702007

				277.4		1.702007

				277.42		1.702007

				277.44		1.697945

				277.46		1.697945

				277.48		1.697945

				277.5		1.697945

				277.53		1.697945

				277.55		1.697945

				277.57		1.697945

				277.59		1.697945

				277.61		1.697945

				277.63		1.697945

				277.65		1.697945

				277.67		1.697945

				277.69		1.697945

				277.71		1.697945

				277.73		1.693883

				277.76		1.693883

				277.78		1.693883

				277.8		1.693883

				277.82		1.693883

				277.84		1.693883

				277.86		1.693883

				277.88		1.693883

				277.9		1.693883

				277.92		1.693883

				277.94		1.693883

				277.97		1.693883

				277.99		1.693883

				278.01		1.693883

				278.03		1.693883

				278.05		1.693883

				278.07		1.68982

				278.09		1.693883

				278.11		1.68982

				278.13		1.68982

				278.15		1.68982

				278.17		1.68982

				278.2		1.68982

				278.22		1.68982

				278.24		1.68982

				278.26		1.68982

				278.28		1.68982

				278.3		1.68982

				278.32		1.68982

				278.34		1.68982

				278.36		1.68982

				278.38		1.68982

				278.41		1.68982

				278.43		1.68982

				278.45		1.685758

				278.47		1.685758

				278.49		1.685758

				278.51		1.685758

				278.53		1.685758

				278.55		1.685758

				278.57		1.685758

				278.59		1.685758

				278.61		1.685758

				278.64		1.685758

				278.66		1.685758

				278.68		1.685758

				278.7		1.685758

				278.72		1.685758

				278.74		1.685758

				278.76		1.685758

				278.78		1.685758

				278.8		1.685758

				278.82		1.685758

				278.85		1.685758

				278.87		1.685758

				278.89		1.685758

				278.91		1.685758

				278.93		1.685758

				278.95		1.685758

				278.97		1.685758

				278.99		1.685758

				279.01		1.681696

				279.03		1.681696

				279.05		1.681696

				279.08		1.681696

				279.1		1.681696

				279.12		1.681696

				279.14		1.681696

				279.16		1.681696

				279.18		1.681696

				279.2		1.681696

				279.22		1.681696

				279.24		1.681696

				279.26		1.681696

				279.29		1.681696

				279.31		1.681696

				279.33		1.677634

				279.35		1.681696

				279.37		1.677634

				279.39		1.677634

				279.41		1.677634

				279.43		1.677634

				279.45		1.677634

				279.47		1.677634

				279.49		1.677634

				279.52		1.677634

				279.54		1.677634

				279.56		1.677634

				279.58		1.677634

				279.6		1.677634

				279.62		1.677634

				279.64		1.677634

				279.66		1.677634

				279.68		1.677634

				279.7		1.677634

				279.73		1.677634

				279.75		1.677634

				279.77		1.677634

				279.79		1.677634

				279.81		1.677634

				279.83		1.677634

				279.85		1.677634

				279.87		1.677634

				279.89		1.677634

				279.91		1.677634

				279.94		1.677634

				279.96		1.677634

				279.98		1.677634

				280		1.677634

				280.02		1.677634

				280.04		1.677634

				280.06		1.677634

				280.08		1.673572

				280.1		1.673572

				280.12		1.673572

				280.14		1.673572

				280.17		1.673572

				280.19		1.673572

				280.21		1.673572

				280.23		1.673572

				280.25		1.673572

				280.27		1.673572

				280.29		1.673572

				280.31		1.673572

				280.33		1.673572

				280.35		1.673572

				280.38		1.673572

				280.4		1.673572

				280.42		1.673572

				280.44		1.673572

				280.46		1.673572

				280.48		1.673572

				280.5		1.673572

				280.52		1.673572

				280.54		1.673572

				280.56		1.673572

				280.59		1.673572

				280.61		1.673572

				280.63		1.673572

				280.65		1.673572

				280.67		1.673572

				280.69		1.673572

				280.71		1.673572

				280.73		1.673572

				280.75		1.673572

				280.77		1.673572

				280.79		1.673572

				280.82		1.673572

				280.84		1.673572

				280.86		1.66951

				280.88		1.66951

				280.9		1.66951

				280.92		1.66951

				280.94		1.66951

				280.96		1.66951

				280.98		1.66951

				281		1.66951

				281.03		1.66951

				281.05		1.66951

				281.07		1.66951

				281.09		1.66951

				281.11		1.66951

				281.13		1.66951

				281.15		1.66951

				281.17		1.66951

				281.19		1.66951

				281.21		1.66951

				281.24		1.66951

				281.26		1.66951

				281.28		1.66951

				281.3		1.66951

				281.32		1.66951

				281.34		1.66951

				281.36		1.66951

				281.38		1.66951

				281.4		1.66951

				281.42		1.66951

				281.45		1.66951

				281.47		1.66951

				281.49		1.66951

				281.51		1.66951

				281.53		1.66951

				281.55		1.66951

				281.57		1.66951

				281.59		1.665448

				281.61		1.66951

				281.63		1.665448

				281.65		1.66951

				281.68		1.665448

				281.7		1.665448

				281.72		1.665448

				281.74		1.665448

				281.76		1.665448

				281.78		1.665448

				281.8		1.665448

				281.82		1.665448

				281.84		1.665448

				281.86		1.665448

				281.89		1.665448

				281.91		1.665448

				281.93		1.665448

				281.95		1.665448

				281.97		1.665448

				281.99		1.665448

				282.01		1.665448

				282.03		1.665448

				282.05		1.665448

				282.07		1.665448

				282.1		1.665448

				282.12		1.665448

				282.14		1.665448

				282.16		1.665448

				282.18		1.665448

				282.2		1.665448

				282.22		1.665448

				282.24		1.665448

				282.26		1.665448

				282.28		1.665448

				282.3		1.665448

				282.33		1.665448

				282.35		1.665448

				282.37		1.665448

				282.39		1.665448

				282.41		1.665448

				282.43		1.665448

				282.45		1.665448

				282.47		1.665448

				282.49		1.665448

				282.51		1.665448

				282.54		1.665448

				282.56		1.665448

				282.58		1.665448

				282.6		1.665448

				282.62		1.665448

				282.64		1.665448

				282.66		1.665448

				282.68		1.665448

				282.7		1.665448

				282.72		1.665448

				282.75		1.665448

				282.77		1.665448

				282.79		1.665448

				282.81		1.665448

				282.83		1.665448

				282.85		1.661386

				282.87		1.661386

				282.89		1.661386

				282.91		1.661386

				282.93		1.661386

				282.96		1.661386

				282.98		1.661386

				283		1.661386

				283.02		1.661386

				283.04		1.661386

				283.06		1.661386

				283.08		1.661386

				283.1		1.661386

				283.12		1.661386

				283.14		1.661386

				283.17		1.661386

				283.19		1.661386

				283.21		1.661386

				283.23		1.661386

				283.25		1.661386

				283.27		1.661386

				283.29		1.661386

				283.31		1.661386

				283.33		1.661386

				283.35		1.661386

				283.37		1.661386

				283.4		1.661386

				283.42		1.661386

				283.44		1.661386

				283.46		1.661386

				283.48		1.661386

				283.5		1.661386

				283.52		1.661386

				283.54		1.661386

				283.56		1.661386

				283.58		1.661386

				283.61		1.661386

				283.63		1.661386

				283.65		1.661386

				283.67		1.661386

				283.69		1.661386

				283.71		1.661386

				283.73		1.661386

				283.75		1.657324

				283.77		1.657324

				283.79		1.657324

				283.82		1.657324

				283.84		1.661386

				283.86		1.661386

				283.88		1.661386

				283.9		1.661386

				283.92		1.661386

				283.94		1.661386

				283.96		1.661386

				283.98		1.661386

				284		1.661386

				284.03		1.661386

				284.05		1.657324

				284.07		1.657324

				284.09		1.657324

				284.11		1.657324

				284.13		1.657324

				284.15		1.657324

				284.17		1.657324

				284.19		1.657324

				284.21		1.657324

				284.24		1.657324

				284.26		1.657324

				284.28		1.657324

				284.3		1.657324

				284.32		1.657324

				284.34		1.657324

				284.36		1.657324

				284.38		1.657324

				284.4		1.657324

				284.42		1.657324

				284.45		1.657324

				284.47		1.653262

				284.49		1.653262

				284.51		1.653262

				284.53		1.653262

				284.55		1.653262

				284.57		1.653262

				284.59		1.653262

				284.61		1.653262

				284.64		1.653262

				284.66		1.653262

				284.68		1.653262

				284.7		1.653262

				284.72		1.653262

				284.74		1.653262

				284.76		1.653262

				284.78		1.653262

				284.8		1.653262

				284.82		1.653262

				284.85		1.6492

				284.87		1.653262

				284.89		1.6492

				284.91		1.6492

				284.93		1.6492

				284.95		1.6492

				284.97		1.6492

				284.99		1.6492

				285.01		1.6492

				285.03		1.6492

				285.06		1.6492

				285.08		1.6492

				285.1		1.6492

				285.12		1.6492

				285.14		1.6492

				285.16		1.6492

				285.18		1.6492

				285.2		1.6492

				285.22		1.6492

				285.24		1.6492

				285.27		1.6492

				285.29		1.645138

				285.31		1.645138

				285.33		1.645138

				285.35		1.645138

				285.37		1.645138

				285.39		1.645138

				285.41		1.645138

				285.43		1.645138

				285.46		1.645138

				285.48		1.645138

				285.5		1.645138

				285.52		1.645138

				285.54		1.645138

				285.56		1.645138

				285.58		1.645138

				285.6		1.645138

				285.62		1.645138

				285.64		1.645138

				285.67		1.641076

				285.69		1.641076

				285.71		1.641076

				285.73		1.641076

				285.75		1.641076

				285.77		1.641076

				285.79		1.641076

				285.81		1.641076

				285.83		1.641076

				285.86		1.641076

				285.88		1.641076

				285.9		1.641076

				285.92		1.641076

				285.94		1.637014

				285.96		1.637014

				285.98		1.637014

				286		1.637014

				286.02		1.637014

				286.04		1.637014

				286.07		1.637014

				286.09		1.637014

				286.11		1.637014

				286.13		1.637014

				286.15		1.637014

				286.17		1.637014

				286.19		1.637014

				286.21		1.637014

				286.23		1.637014

				286.26		1.637014

				286.28		1.637014

				286.3		1.637014

				286.32		1.637014

				286.34		1.637014

				286.36		1.637014

				286.38		1.637014

				286.4		1.637014

				286.42		1.637014

				286.44		1.637014

				286.47		1.637014

				286.49		1.637014

				286.51		1.637014

				286.53		1.632951

				286.55		1.637014

				286.57		1.632951

				286.59		1.632951

				286.61		1.632951

				286.63		1.632951

				286.66		1.632951

				286.68		1.632951

				286.7		1.632951

				286.72		1.632951

				286.74		1.632951

				286.76		1.632951

				286.78		1.632951

				286.8		1.632951

				286.82		1.632951

				286.85		1.632951

				286.87		1.632951

				286.89		1.632951

				286.91		1.632951

				286.93		1.632951

				286.95		1.632951

				286.97		1.632951

				286.99		1.632951

				287.01		1.632951

				287.04		1.632951

				287.06		1.632951

				287.08		1.632951

				287.1		1.632951

				287.12		1.632951

				287.14		1.632951

				287.16		1.632951

				287.18		1.632951

				287.2		1.632951

				287.22		1.632951

				287.25		1.632951

				287.27		1.632951

				287.29		1.632951

				287.31		1.632951

				287.33		1.632951

				287.35		1.632951

				287.37		1.632951

				287.39		1.632951

				287.41		1.632951

				287.44		1.632951

				287.46		1.632951

				287.48		1.632951

				287.5		1.632951

				287.52		1.632951

				287.54		1.632951

				287.56		1.632951

				287.58		1.632951

				287.6		1.632951

				287.62		1.632951

				287.65		1.632951

				287.67		1.632951

				287.69		1.632951

				287.71		1.632951

				287.73		1.632951

				287.75		1.632951

				287.77		1.632951

				287.79		1.632951

				287.81		1.632951

				287.84		1.632951

				287.86		1.632951

				287.88		1.632951

				287.9		1.632951

				287.92		1.632951

				287.94		1.632951

				287.96		1.632951

				287.98		1.632951

				288		1.632951

				288.02		1.632951

				288.05		1.632951

				288.07		1.632951

				288.09		1.632951

				288.11		1.632951

				288.13		1.632951

				288.15		1.632951

				288.17		1.632951

				288.19		1.628889

				288.21		1.628889

				288.23		1.628889

				288.26		1.628889

				288.28		1.628889

				288.3		1.628889

				288.32		1.628889

				288.34		1.628889

				288.36		1.628889

				288.38		1.628889

				288.4		1.628889

				288.42		1.628889

				288.45		1.628889

				288.47		1.628889

				288.49		1.628889

				288.51		1.628889

				288.53		1.628889

				288.55		1.628889

				288.57		1.628889

				288.59		1.628889

				288.61		1.628889

				288.64		1.628889

				288.66		1.628889

				288.68		1.628889

				288.7		1.628889

				288.72		1.624827

				288.74		1.624827

				288.76		1.628889

				288.78		1.624827

				288.8		1.628889

				288.82		1.624827

				288.85		1.624827

				288.87		1.624827

				288.89		1.624827

				288.91		1.624827

				288.93		1.624827

				288.95		1.624827

				288.97		1.624827

				288.99		1.624827

				289.01		1.624827

				289.04		1.624827

				289.06		1.624827

				289.08		1.624827

				289.1		1.624827

				289.12		1.624827

				289.14		1.624827

				289.16		1.624827

				289.18		1.624827

				289.2		1.624827

				289.23		1.620765

				289.25		1.620765

				289.27		1.620765

				289.29		1.620765

				289.31		1.620765

				289.33		1.620765

				289.35		1.620765

				289.37		1.620765

				289.39		1.620765

				289.42		1.620765

				289.44		1.620765

				289.46		1.620765

				289.48		1.620765

				289.5		1.620765

				289.52		1.620765

				289.54		1.620765

				289.56		1.620765

				289.58		1.620765

				289.6		1.620765

				289.63		1.620765

				289.65		1.620765

				289.67		1.620765

				289.69		1.620765

				289.71		1.620765

				289.73		1.620765

				289.75		1.620765

				289.77		1.620765

				289.79		1.620765

				289.82		1.620765

				289.84		1.620765

				289.86		1.620765

				289.88		1.620765

				289.9		1.620765

				289.92		1.620765

				289.94		1.616703

				289.96		1.620765

				289.98		1.620765

				290.01		1.616703

				290.03		1.620765

				290.05		1.616703

				290.07		1.616703

				290.09		1.616703

				290.11		1.616703

				290.13		1.616703

				290.15		1.616703

				290.17		1.616703

				290.2		1.616703

				290.22		1.616703

				290.24		1.616703

				290.26		1.616703

				290.28		1.616703

				290.3		1.616703

				290.32		1.616703

				290.34		1.616703

				290.36		1.616703

				290.38		1.616703

				290.41		1.616703

				290.43		1.616703

				290.45		1.616703

				290.47		1.616703

				290.49		1.616703

				290.51		1.616703

				290.53		1.616703

				290.55		1.616703

				290.57		1.616703

				290.6		1.616703

				290.62		1.616703

				290.64		1.616703

				290.66		1.616703

				290.68		1.616703

				290.7		1.616703

				290.72		1.616703

				290.74		1.616703

				290.76		1.616703

				290.79		1.616703

				290.81		1.616703

				290.83		1.616703

				290.85		1.612641

				290.87		1.612641

				290.89		1.612641

				290.91		1.612641

				290.93		1.612641

				290.95		1.612641

				290.97		1.612641

				291		1.612641

				291.02		1.612641

				291.04		1.612641

				291.06		1.612641

				291.08		1.612641

				291.1		1.612641

				291.12		1.612641

				291.14		1.612641

				291.16		1.612641

				291.19		1.612641

				291.21		1.612641

				291.23		1.612641

				291.25		1.612641

				291.27		1.612641

				291.29		1.612641

				291.31		1.612641

				291.33		1.608579

				291.35		1.608579

				291.38		1.608579

				291.4		1.608579

				291.42		1.608579

				291.44		1.608579

				291.46		1.608579

				291.48		1.608579

				291.5		1.608579

				291.52		1.608579

				291.54		1.608579

				291.57		1.608579

				291.59		1.608579

				291.61		1.608579

				291.63		1.608579

				291.65		1.608579

				291.67		1.608579

				291.69		1.608579

				291.71		1.608579

				291.73		1.608579

				291.76		1.608579

				291.78		1.608579

				291.8		1.608579

				291.82		1.608579

				291.84		1.608579

				291.86		1.608579

				291.88		1.608579

				291.9		1.608579

				291.92		1.608579

				291.95		1.604517

				291.97		1.604517

				291.99		1.604517

				292.01		1.604517

				292.03		1.608579

				292.05		1.604517

				292.07		1.604517

				292.09		1.608579

				292.11		1.604517

				292.13		1.604517

				292.16		1.604517

				292.18		1.604517

				292.2		1.604517

				292.22		1.604517

				292.24		1.604517

				292.26		1.604517

				292.28		1.604517

				292.3		1.604517

				292.32		1.604517

				292.35		1.604517

				292.37		1.604517

				292.39		1.604517

				292.41		1.604517

				292.43		1.604517

				292.45		1.604517

				292.47		1.604517

				292.49		1.604517

				292.51		1.604517

				292.54		1.604517

				292.56		1.604517

				292.58		1.604517

				292.6		1.604517

				292.62		1.604517

				292.64		1.604517

				292.66		1.604517

				292.68		1.604517

				292.7		1.604517

				292.73		1.604517

				292.75		1.604517

				292.77		1.604517

				292.79		1.604517

				292.81		1.604517

				292.83		1.604517

				292.85		1.604517

				292.87		1.604517

				292.89		1.604517

				292.91		1.604517

				292.94		1.604517

				292.96		1.604517

				292.98		1.604517

				293		1.604517

				293.02		1.604517

				293.04		1.608579

				293.06		1.604517

				293.08		1.608579

				293.1		1.608579

				293.13		1.608579

				293.15		1.608579

				293.17		1.608579

				293.19		1.608579

				293.21		1.608579

				293.23		1.608579

				293.25		1.608579

				293.27		1.608579

				293.29		1.608579

				293.32		1.608579

				293.34		1.608579

				293.36		1.608579

				293.38		1.608579

				293.4		1.608579

				293.42		1.608579

				293.44		1.608579

				293.46		1.608579

				293.48		1.608579

				293.5		1.608579

				293.53		1.608579

				293.55		1.608579

				293.57		1.608579

				293.59		1.608579

				293.61		1.608579

				293.63		1.608579

				293.65		1.608579

				293.67		1.608579

				293.69		1.608579

				293.72		1.604517

				293.74		1.604517

				293.76		1.604517

				293.78		1.604517

				293.8		1.604517

				293.82		1.604517

				293.84		1.604517

				293.86		1.604517

				293.88		1.604517

				293.91		1.604517

				293.93		1.604517

				293.95		1.604517

				293.97		1.604517

				293.99		1.604517

				294.01		1.604517

				294.03		1.604517

				294.05		1.604517

				294.07		1.604517

				294.09		1.604517

				294.12		1.604517

				294.14		1.604517

				294.16		1.600455

				294.18		1.600455

				294.2		1.604517

				294.22		1.600455

				294.24		1.600455

				294.26		1.600455

				294.28		1.600455

				294.31		1.600455

				294.33		1.600455

				294.35		1.600455

				294.37		1.600455

				294.39		1.600455

				294.41		1.600455

				294.43		1.600455

				294.45		1.600455

				294.47		1.600455

				294.5		1.600455

				294.52		1.600455

				294.54		1.600455

				294.56		1.600455

				294.58		1.600455

				294.6		1.600455

				294.62		1.600455

				294.64		1.600455

				294.66		1.600455

				294.69		1.600455

				294.71		1.600455

				294.73		1.600455

				294.75		1.596393

				294.77		1.596393

				294.79		1.596393

				294.81		1.596393

				294.83		1.596393

				294.85		1.596393

				294.88		1.596393

				294.9		1.596393

				294.92		1.596393

				294.94		1.596393

				294.96		1.596393

				294.98		1.596393

				295		1.596393

				295.02		1.596393

				295.04		1.596393

				295.07		1.596393

				295.09		1.596393

				295.11		1.596393

				295.13		1.596393

				295.15		1.596393

				295.17		1.596393

				295.19		1.592331

				295.21		1.592331

				295.23		1.592331

				295.26		1.592331

				295.28		1.592331

				295.3		1.592331

				295.32		1.592331

				295.34		1.592331

				295.36		1.592331

				295.38		1.592331

				295.4		1.592331

				295.42		1.592331

				295.45		1.592331

				295.47		1.592331

				295.49		1.592331

				295.51		1.592331

				295.53		1.592331

				295.55		1.592331

				295.57		1.592331

				295.59		1.592331

				295.61		1.592331

				295.63		1.592331

				295.66		1.592331

				295.68		1.592331

				295.7		1.592331

				295.72		1.592331

				295.74		1.592331

				295.76		1.592331

				295.78		1.592331

				295.8		1.592331

				295.82		1.592331

				295.85		1.592331

				295.87		1.592331

				295.89		1.592331

				295.91		1.592331

				295.93		1.596393

				295.95		1.596393

				295.97		1.596393

				295.99		1.596393

				296.01		1.596393

				296.04		1.596393

				296.06		1.596393

				296.08		1.596393

				296.1		1.596393

				296.12		1.596393

				296.14		1.596393

				296.16		1.596393

				296.18		1.592331

				296.2		1.592331

				296.23		1.592331

				296.25		1.596393

				296.27		1.592331

				296.29		1.592331

				296.31		1.592331

				296.33		1.592331

				296.35		1.592331

				296.37		1.592331

				296.39		1.592331

				296.41		1.596393

				296.44		1.596393

				296.46		1.596393

				296.48		1.596393

				296.5		1.596393

				296.52		1.596393

				296.54		1.596393

				296.56		1.596393

				296.58		1.596393

				296.6		1.596393

				296.63		1.596393

				296.65		1.596393

				296.67		1.596393

				296.69		1.596393

				296.71		1.596393

				296.73		1.596393

				296.75		1.596393

				296.77		1.596393

				296.79		1.596393

				296.82		1.596393

				296.84		1.596393

				296.86		1.596393

				296.88		1.596393

				296.9		1.596393

				296.92		1.596393

				296.94		1.596393

				296.96		1.596393

				296.98		1.596393

				297.01		1.596393

				297.03		1.596393

				297.05		1.596393

				297.07		1.596393

				297.09		1.596393

				297.11		1.596393

				297.13		1.596393

				297.15		1.596393

				297.17		1.592331

				297.2		1.592331

				297.22		1.592331

				297.24		1.592331

				297.26		1.592331

				297.28		1.592331

				297.3		1.592331

				297.32		1.592331

				297.34		1.592331

				297.36		1.592331

				297.38		1.592331

				297.41		1.592331

				297.43		1.592331

				297.45		1.592331

				297.47		1.592331

				297.49		1.592331

				297.51		1.592331

				297.53		1.592331

				297.55		1.592331

				297.57		1.592331

				297.6		1.592331

				297.62		1.592331

				297.64		1.592331

				297.66		1.592331

				297.68		1.592331

				297.7		1.592331

				297.72		1.592331

				297.74		1.592331

				297.76		1.588269

				297.79		1.588269

				297.81		1.592331

				297.83		1.592331

				297.85		1.592331

				297.87		1.592331

				297.89		1.592331

				297.91		1.588269

				297.93		1.592331

				297.95		1.592331

				297.98		1.588269

				298		1.588269

				298.02		1.588269

				298.04		1.588269

				298.06		1.588269

				298.08		1.588269

				298.1		1.588269

				298.12		1.588269

				298.14		1.588269

				298.17		1.588269

				298.19		1.588269

				298.21		1.588269

				298.23		1.588269

				298.25		1.588269

				298.27		1.588269

				298.29		1.588269

				298.31		1.588269

				298.33		1.588269

				298.36		1.588269

				298.38		1.588269

				298.4		1.588269

				298.42		1.588269

				298.44		1.588269

				298.46		1.588269

				298.48		1.588269

				298.5		1.588269

				298.52		1.588269

				298.54		1.588269

				298.57		1.588269

				298.59		1.588269

				298.61		1.584207

				298.63		1.588269

				298.65		1.588269

				298.67		1.588269

				298.69		1.584207

				298.71		1.584207

				298.73		1.584207

				298.76		1.588269

				298.78		1.584207

				298.8		1.588269

				298.82		1.584207

				298.84		1.588269

				298.86		1.588269

				298.88		1.584207

				298.9		1.584207

				298.92		1.584207

				298.95		1.584207

				298.97		1.584207

				298.99		1.588269

				299.01		1.588269

				299.03		1.584207

				299.05		1.584207

				299.07		1.588269

				299.09		1.588269

				299.11		1.588269

				299.14		1.588269

				299.16		1.588269

				299.18		1.588269

				299.2		1.588269

				299.22		1.588269

				299.24		1.588269

				299.26		1.588269

				299.28		1.588269

				299.3		1.588269

				299.33		1.588269

				299.35		1.588269

				299.37		1.588269

				299.39		1.588269

				299.41		1.588269

				299.43		1.588269

				299.45		1.588269

				299.47		1.588269

				299.49		1.588269

				299.52		1.588269

				299.54		1.588269

				299.56		1.588269

				299.58		1.588269

				299.6		1.588269

				299.62		1.588269

				299.64		1.588269

				299.66		1.588269

				299.68		1.588269

				299.71		1.588269

				299.73		1.588269

				299.75		1.588269

				299.77		1.588269

				299.79		1.588269

				299.81		1.588269

				299.83		1.588269

				299.85		1.588269

				299.87		1.588269

				299.9		1.588269

				299.92		1.588269

				299.94		1.588269

				299.96		1.588269

				299.98		1.588269

				300		1.588269

				300.02		1.588269

				300.04		1.588269

				300.06		1.588269

				300.09		1.588269

				300.11		1.588269

				300.13		1.588269

				300.15		1.588269

				300.17		1.588269

				300.19		1.588269

				300.21		1.588269

				300.23		1.588269

				300.25		1.588269

				300.28		1.588269

				300.3		1.588269

				300.32		1.588269

				300.34		1.588269

				300.36		1.588269

				300.38		1.588269

				300.4		1.588269

				300.42		1.588269

				300.44		1.588269

				300.47		1.588269

				300.49		1.588269

				300.51		1.588269

				300.53		1.588269

				300.55		1.588269

				300.57		1.588269

				300.59		1.588269

				300.61		1.588269

				300.63		1.588269

				300.65		1.588269

				300.68		1.588269

				300.7		1.588269

				300.72		1.588269

				300.74		1.588269

				300.76		1.588269

				300.78		1.588269

				300.8		1.588269

				300.82		1.588269

				300.84		1.588269

				300.87		1.588269

				300.89		1.588269

				300.91		1.588269

				300.93		1.588269

				300.95		1.588269

				300.97		1.588269

				300.99		1.588269

				301.01		1.588269

				301.03		1.588269

				301.06		1.588269

				301.08		1.584207

				301.1		1.584207

				301.12		1.588269

				301.14		1.584207

				301.16		1.584207

				301.18		1.584207

				301.2		1.584207

				301.22		1.584207

				301.25		1.584207

				301.27		1.584207

				301.29		1.584207

				301.31		1.584207

				301.33		1.584207

				301.35		1.584207

				301.37		1.584207

				301.39		1.584207

				301.41		1.584207

				301.44		1.584207

				301.46		1.584207

				301.48		1.584207

				301.5		1.584207

				301.52		1.584207

				301.54		1.588269

				301.56		1.584207

				301.58		1.588269

				301.6		1.588269

				301.63		1.588269

				301.65		1.588269

				301.67		1.588269

				301.69		1.588269

				301.71		1.588269

				301.73		1.588269

				301.75		1.588269

				301.77		1.588269

				301.79		1.588269

				301.81		1.588269

				301.84		1.588269

				301.86		1.588269

				301.88		1.588269

				301.9		1.588269

				301.92		1.588269

				301.94		1.588269

				301.96		1.588269

				301.98		1.588269

				302		1.588269

				302.03		1.588269

				302.05		1.588269

				302.07		1.588269

				302.09		1.588269

				302.11		1.588269

				302.13		1.588269

				302.15		1.588269

				302.17		1.588269

				302.19		1.588269

				302.22		1.588269

				302.24		1.588269

				302.26		1.588269

				302.28		1.588269

				302.3		1.588269

				302.32		1.588269

				302.34		1.588269

				302.36		1.588269

				302.38		1.588269

				302.41		1.588269

				302.43		1.588269

				302.45		1.588269

				302.47		1.588269

				302.49		1.588269

				302.51		1.588269

				302.53		1.588269

				302.55		1.588269

				302.57		1.588269

				302.6		1.588269

				302.62		1.588269

				302.64		1.588269

				302.66		1.588269

				302.68		1.588269

				302.7		1.588269

				302.72		1.588269

				302.74		1.592331

				302.76		1.592331

				302.79		1.592331

				302.81		1.592331

				302.83		1.592331

				302.85		1.592331

				302.87		1.592331

				302.89		1.592331

				302.91		1.592331

				302.93		1.592331

				302.95		1.588269

				302.98		1.592331

				303		1.588269

				303.02		1.592331

				303.04		1.592331

				303.06		1.592331

				303.08		1.588269

				303.1		1.592331

				303.12		1.592331

				303.14		1.592331

				303.17		1.592331

				303.19		1.592331

				303.21		1.592331

				303.23		1.588269

				303.25		1.588269

				303.27		1.588269

				303.29		1.588269

				303.31		1.588269

				303.33		1.588269

				303.36		1.588269

				303.38		1.588269

				303.4		1.588269

				303.42		1.588269

				303.44		1.588269

				303.46		1.588269

				303.48		1.588269

				303.5		1.588269

				303.52		1.588269

				303.55		1.588269

				303.57		1.588269

				303.59		1.588269

				303.61		1.588269

				303.63		1.588269

				303.65		1.588269

				303.67		1.588269

				303.69		1.588269

				303.71		1.588269

				303.74		1.588269

				303.76		1.584207

				303.78		1.584207

				303.8		1.584207

				303.82		1.584207

				303.84		1.584207

				303.86		1.584207

				303.88		1.584207

				303.9		1.584207

				303.92		1.584207

				303.95		1.584207

				303.97		1.584207

				303.99		1.584207

				304.01		1.584207

				304.03		1.584207

				304.05		1.584207

				304.07		1.584207

				304.09		1.584207

				304.11		1.584207

				304.14		1.584207

				304.16		1.584207

				304.18		1.584207

				304.2		1.580145

				304.22		1.580145

				304.24		1.580145

				304.26		1.580145

				304.28		1.580145

				304.3		1.580145

				304.33		1.580145

				304.35		1.580145

				304.37		1.580145

				304.39		1.580145

				304.41		1.580145

				304.43		1.580145

				304.45		1.580145

				304.47		1.580145

				304.49		1.580145

				304.52		1.580145

				304.54		1.580145

				304.56		1.580145

				304.58		1.580145

				304.6		1.580145

				304.62		1.580145

				304.64		1.580145

				304.66		1.580145

				304.68		1.580145

				304.71		1.580145

				304.73		1.580145

				304.75		1.580145

				304.77		1.580145

				304.79		1.580145

				304.81		1.580145

				304.83		1.580145

				304.85		1.580145

				304.87		1.576083

				304.89		1.576083

				304.92		1.576083

				304.94		1.576083

				304.96		1.580145

				304.98		1.576083

				305		1.576083

				305.02		1.576083

				305.04		1.576083

				305.06		1.576083

				305.08		1.576083

				305.11		1.576083

				305.13		1.576083

				305.15		1.576083

				305.17		1.576083

				305.19		1.576083

				305.21		1.576083

				305.23		1.576083

				305.25		1.576083

				305.27		1.576083

				305.3		1.576083

				305.32		1.576083

				305.34		1.576083

				305.36		1.576083

				305.38		1.576083

				305.4		1.576083

				305.42		1.576083

				305.44		1.576083

				305.46		1.576083

				305.49		1.576083

				305.51		1.576083

				305.53		1.576083

				305.55		1.576083

				305.57		1.576083

				305.59		1.576083

				305.61		1.576083

				305.63		1.576083

				305.65		1.576083

				305.68		1.576083

				305.7		1.576083

				305.72		1.576083

				305.74		1.576083

				305.76		1.576083

				305.78		1.576083

				305.8		1.576083

				305.82		1.576083

				305.84		1.576083

				305.87		1.576083

				305.89		1.576083

				305.91		1.576083

				305.93		1.57202

				305.95		1.576083

				305.97		1.57202

				305.99		1.57202

				306.01		1.57202

				306.03		1.57202

				306.06		1.57202

				306.08		1.57202

				306.1		1.57202

				306.12		1.57202

				306.14		1.57202

				306.16		1.57202

				306.18		1.57202

				306.2		1.57202

				306.22		1.57202

				306.25		1.57202

				306.27		1.57202

				306.29		1.57202

				306.31		1.57202

				306.33		1.567958

				306.35		1.567958

				306.37		1.567958

				306.39		1.567958

				306.41		1.567958

				306.44		1.567958

				306.46		1.567958

				306.48		1.567958

				306.5		1.567958

				306.52		1.563896

				306.54		1.567958

				306.56		1.563896

				306.58		1.563896

				306.6		1.563896

				306.63		1.563896

				306.65		1.563896

				306.67		1.563896

				306.69		1.563896

				306.71		1.563896

				306.73		1.563896

				306.75		1.563896

				306.77		1.563896

				306.79		1.563896

				306.82		1.563896

				306.84		1.563896

				306.86		1.563896

				306.88		1.563896

				306.9		1.563896

				306.92		1.563896

				306.94		1.563896

				306.96		1.563896

				306.99		1.563896

				307.01		1.563896

				307.03		1.563896

				307.05		1.559834

				307.07		1.559834

				307.09		1.559834

				307.11		1.559834

				307.13		1.559834

				307.15		1.559834

				307.18		1.559834

				307.2		1.559834

				307.22		1.559834

				307.24		1.559834

				307.26		1.559834

				307.28		1.559834

				307.3		1.559834

				307.32		1.559834

				307.34		1.559834

				307.37		1.559834

				307.39		1.559834

				307.41		1.559834

				307.43		1.559834

				307.45		1.559834

				307.47		1.559834

				307.49		1.559834

				307.51		1.559834

				307.53		1.559834

				307.56		1.559834

				307.58		1.559834

				307.6		1.559834

				307.62		1.559834

				307.64		1.559834

				307.66		1.559834

				307.68		1.559834

				307.7		1.559834

				307.72		1.559834

				307.75		1.559834

				307.77		1.559834

				307.79		1.559834

				307.81		1.559834

				307.83		1.559834

				307.85		1.559834

				307.87		1.559834

				307.89		1.559834

				307.92		1.559834

				307.94		1.559834

				307.96		1.559834

				307.98		1.559834

				308		1.559834

				308.02		1.559834

				308.04		1.559834

				308.06		1.559834

				308.08		1.559834

				308.11		1.559834

				308.13		1.559834

				308.15		1.559834

				308.17		1.559834

				308.19		1.559834

				308.21		1.559834

				308.23		1.559834

				308.25		1.559834

				308.27		1.559834

				308.3		1.559834

				308.32		1.559834

				308.34		1.559834

				308.36		1.559834

				308.38		1.559834

				308.4		1.559834

				308.42		1.559834

				308.44		1.559834

				308.46		1.559834

				308.49		1.559834

				308.51		1.559834

				308.53		1.559834

				308.55		1.559834

				308.57		1.559834

				308.59		1.559834

				308.61		1.559834

				308.63		1.559834

				308.65		1.559834

				308.68		1.559834

				308.7		1.559834

				308.72		1.559834

				308.74		1.559834

				308.76		1.559834

				308.78		1.559834

				308.8		1.559834

				308.82		1.559834

				308.84		1.559834

				308.87		1.559834

				308.89		1.559834

				308.91		1.559834

				308.93		1.559834

				308.95		1.559834

				308.97		1.559834

				308.99		1.559834

				309.01		1.559834

				309.04		1.559834

				309.06		1.559834

				309.08		1.559834

				309.1		1.559834

				309.12		1.559834

				309.14		1.559834

				309.16		1.559834

				309.18		1.559834

				309.2		1.559834

				309.23		1.559834

				309.25		1.559834

				309.27		1.559834

				309.29		1.559834

				309.31		1.559834

				309.33		1.559834

				309.35		1.559834

				309.37		1.559834

				309.39		1.559834

				309.42		1.559834

				309.44		1.559834

				309.46		1.559834

				309.48		1.559834

				309.5		1.559834

				309.52		1.559834

				309.54		1.559834

				309.56		1.559834

				309.58		1.559834

				309.61		1.559834

				309.63		1.559834

				309.65		1.559834

				309.67		1.559834

				309.69		1.559834

				309.71		1.559834

				309.73		1.559834

				309.75		1.559834

				309.77		1.559834

				309.8		1.559834

				309.82		1.559834

				309.84		1.559834

				309.86		1.559834

				309.88		1.559834

				309.9		1.559834

				309.92		1.559834

				309.94		1.559834

				309.96		1.559834

				309.99		1.559834

				310.01		1.559834

				310.03		1.559834

				310.05		1.559834

				310.07		1.559834

				310.09		1.559834

				310.11		1.559834

				310.13		1.559834

				310.15		1.559834

				310.18		1.559834

				310.2		1.559834

				310.22		1.559834

				310.24		1.559834

				310.26		1.559834

				310.28		1.559834

				310.3		1.559834

				310.32		1.559834

				310.34		1.559834

				310.37		1.559834

				310.39		1.559834

				310.41		1.559834

				310.43		1.559834

				310.45		1.559834

				310.47		1.559834

				310.49		1.559834

				310.51		1.559834

				310.53		1.559834

				310.56		1.559834

				310.58		1.559834

				310.6		1.559834

				310.62		1.559834

				310.64		1.559834

				310.66		1.559834

				310.68		1.559834

				310.7		1.559834

				310.72		1.559834

				310.75		1.559834

				310.77		1.559834

				310.79		1.559834

				310.81		1.559834

				310.83		1.559834

				310.85		1.559834

				310.87		1.559834

				310.89		1.559834

				310.92		1.559834

				310.94		1.559834

				310.96		1.559834

				310.98		1.559834

				311		1.559834

				311.02		1.559834

				311.04		1.559834

				311.06		1.559834

				311.08		1.559834

				311.11		1.559834

				311.13		1.559834

				311.15		1.559834

				311.17		1.559834

				311.19		1.559834

				311.21		1.559834

				311.23		1.555772

				311.25		1.559834

				311.27		1.555772

				311.3		1.559834

				311.32		1.559834

				311.34		1.555772

				311.36		1.555772

				311.38		1.555772

				311.4		1.555772

				311.42		1.555772

				311.44		1.555772

				311.46		1.555772

				311.49		1.555772

				311.51		1.555772

				311.53		1.555772

				311.55		1.555772

				311.57		1.555772

				311.59		1.555772

				311.61		1.555772

				311.63		1.555772

				311.65		1.555772

				311.68		1.555772

				311.7		1.555772

				311.72		1.555772

				311.74		1.555772

				311.76		1.555772

				311.78		1.555772

				311.8		1.555772

				311.82		1.555772

				311.85		1.555772

				311.87		1.555772

				311.89		1.555772

				311.91		1.555772

				311.93		1.555772

				311.95		1.555772

				311.97		1.555772

				311.99		1.555772

				312.01		1.555772

				312.04		1.555772

				312.06		1.555772

				312.08		1.555772

				312.1		1.555772

				312.12		1.555772

				312.14		1.555772

				312.16		1.559834

				312.18		1.555772

				312.2		1.559834

				312.23		1.555772

				312.25		1.559834

				312.27		1.559834

				312.29		1.559834

				312.31		1.559834

				312.33		1.559834

				312.35		1.559834

				312.37		1.559834

				312.39		1.559834

				312.42		1.559834

				312.44		1.559834

				312.46		1.559834

				312.48		1.559834

				312.5		1.559834

				312.52		1.559834

				312.54		1.559834

				312.56		1.559834

				312.59		1.559834

				312.61		1.559834

				312.63		1.559834

				312.65		1.559834

				312.67		1.559834

				312.69		1.559834

				312.71		1.559834

				312.73		1.559834

				312.75		1.559834

				312.78		1.559834

				312.8		1.559834

				312.82		1.559834

				312.84		1.559834

				312.86		1.559834

				312.88		1.559834

				312.9		1.559834

				312.92		1.563896

				312.94		1.563896

				312.97		1.563896

				312.99		1.563896

				313.01		1.563896

				313.03		1.563896

				313.05		1.563896

				313.07		1.563896

				313.09		1.563896

				313.11		1.563896

				313.13		1.563896

				313.16		1.559834

				313.18		1.559834

				313.2		1.559834

				313.22		1.563896

				313.24		1.563896

				313.26		1.559834

				313.28		1.563896

				313.3		1.563896

				313.33		1.563896

				313.35		1.563896

				313.37		1.563896

				313.39		1.563896

				313.41		1.563896

				313.43		1.563896

				313.45		1.563896

				313.47		1.563896

				313.49		1.563896

				313.52		1.563896

				313.54		1.563896

				313.56		1.563896

				313.58		1.559834

				313.6		1.559834

				313.62		1.559834

				313.64		1.563896

				313.66		1.563896

				313.68		1.563896

				313.71		1.563896

				313.73		1.563896

				313.75		1.563896

				313.77		1.563896

				313.79		1.563896

				313.81		1.563896

				313.83		1.563896

				313.85		1.563896

				313.87		1.563896

				313.9		1.563896

				313.92		1.563896

				313.94		1.563896

				313.96		1.563896

				313.98		1.563896

				314		1.563896

				314.02		1.563896

				314.04		1.563896

				314.07		1.563896

				314.09		1.563896

				314.11		1.563896

				314.13		1.563896

				314.15		1.563896

				314.17		1.563896

				314.19		1.563896

				314.21		1.563896

				314.23		1.563896

				314.26		1.563896

				314.28		1.563896

				314.3		1.563896

				314.32		1.563896

				314.34		1.559834

				314.36		1.563896

				314.38		1.563896

				314.4		1.559834

				314.43		1.563896

				314.45		1.563896

				314.47		1.563896

				314.49		1.563896

				314.51		1.563896

				314.53		1.563896

				314.55		1.563896

				314.57		1.563896

				314.59		1.559834

				314.62		1.559834

				314.64		1.563896

				314.66		1.563896

				314.68		1.563896

				314.7		1.563896

				314.72		1.563896

				314.74		1.563896

				314.76		1.563896

				314.78		1.563896

				314.81		1.563896

				314.83		1.563896

				314.85		1.563896

				314.87		1.563896

				314.89		1.563896

				314.91		1.563896

				314.93		1.563896

				314.95		1.563896

				314.98		1.563896

				315		1.563896

				315.02		1.563896

				315.04		1.563896

				315.06		1.563896

				315.08		1.563896

				315.1		1.563896

				315.12		1.563896

				315.14		1.563896

				315.17		1.563896

				315.19		1.563896

				315.21		1.563896

				315.23		1.563896

				315.25		1.563896

				315.27		1.563896

				315.29		1.563896

				315.31		1.563896

				315.33		1.563896

				315.36		1.563896

				315.38		1.563896

				315.4		1.563896

				315.42		1.563896

				315.44		1.563896

				315.46		1.563896

				315.48		1.563896

				315.5		1.563896

				315.52		1.563896

				315.55		1.563896

				315.57		1.563896

				315.59		1.563896

				315.61		1.563896

				315.63		1.563896

				315.65		1.563896

				315.67		1.563896

				315.69		1.563896

				315.72		1.563896

				315.74		1.563896

				315.76		1.563896

				315.78		1.563896

				315.8		1.563896

				315.82		1.563896

				315.84		1.563896

				315.86		1.563896

				315.88		1.563896

				315.91		1.563896

				315.93		1.563896

				315.95		1.563896

				315.97		1.563896

				315.99		1.563896

				316.01		1.563896

				316.03		1.563896

				316.05		1.563896

				316.08		1.563896

				316.1		1.563896

				316.12		1.563896

				316.14		1.563896

				316.16		1.563896

				316.18		1.563896

				316.2		1.563896

				316.22		1.563896

				316.24		1.563896

				316.27		1.563896

				316.29		1.563896

				316.31		1.563896

				316.33		1.563896

				316.35		1.563896

				316.37		1.563896

				316.39		1.563896

				316.41		1.563896

				316.44		1.563896

				316.46		1.563896

				316.48		1.563896

				316.5		1.563896

				316.52		1.563896

				316.54		1.563896

				316.56		1.563896

				316.58		1.563896

				316.6		1.563896

				316.63		1.563896

				316.65		1.563896

				316.67		1.563896

				316.69		1.563896

				316.71		1.563896

				316.73		1.563896

				316.75		1.563896

				316.77		1.563896

				316.8		1.563896

				316.82		1.563896

				316.84		1.563896

				316.86		1.563896

				316.88		1.563896

				316.9		1.563896

				316.92		1.563896

				316.94		1.563896

				316.96		1.563896

				316.99		1.563896

				317.01		1.563896

				317.03		1.563896

				317.05		1.559834

				317.07		1.559834

				317.09		1.559834

				317.11		1.559834

				317.13		1.559834

				317.15		1.559834

				317.18		1.559834

				317.2		1.559834

				317.22		1.559834

				317.24		1.559834

				317.26		1.559834

				317.28		1.559834

				317.3		1.559834

				317.32		1.559834

				317.35		1.559834

				317.37		1.559834

				317.39		1.559834

				317.41		1.559834

				317.43		1.559834

				317.45		1.559834

				317.47		1.559834

				317.49		1.559834

				317.51		1.559834

				317.54		1.559834

				317.56		1.559834

				317.58		1.559834

				317.6		1.559834

				317.62		1.559834

				317.64		1.559834

				317.66		1.559834

				317.68		1.559834

				317.7		1.559834

				317.73		1.559834

				317.75		1.559834

				317.77		1.559834

				317.79		1.559834

				317.81		1.559834

				317.83		1.559834

				317.85		1.559834

				317.87		1.559834

				317.9		1.559834

				317.92		1.559834

				317.94		1.555772

				317.96		1.559834

				317.98		1.559834

				318		1.559834

				318.02		1.559834

				318.04		1.555772

				318.06		1.559834

				318.09		1.559834

				318.11		1.555772

				318.13		1.555772

				318.15		1.555772

				318.17		1.555772

				318.19		1.555772

				318.21		1.555772

				318.23		1.555772

				318.25		1.555772

				318.28		1.555772

				318.3		1.555772

				318.32		1.555772

				318.34		1.555772

				318.36		1.555772

				318.38		1.555772

				318.4		1.555772

				318.42		1.555772

				318.45		1.555772

				318.47		1.555772

				318.49		1.555772

				318.51		1.555772

				318.53		1.555772

				318.55		1.555772

				318.57		1.555772

				318.59		1.55171

				318.61		1.555772

				318.64		1.55171

				318.66		1.55171

				318.68		1.55171

				318.7		1.55171

				318.72		1.55171

				318.74		1.55171

				318.76		1.55171

				318.78		1.55171

				318.81		1.55171

				318.83		1.55171

				318.85		1.55171

				318.87		1.55171

				318.89		1.55171

				318.91		1.55171

				318.93		1.55171

				318.95		1.547648

				318.97		1.547648

				319		1.547648

				319.02		1.547648

				319.04		1.547648

				319.06		1.547648

				319.08		1.547648

				319.1		1.547648

				319.12		1.547648

				319.14		1.547648

				319.16		1.547648

				319.19		1.547648

				319.21		1.547648

				319.23		1.547648

				319.25		1.547648

				319.27		1.547648

				319.29		1.547648

				319.31		1.543586

				319.33		1.543586

				319.36		1.543586

				319.38		1.543586

				319.4		1.543586

				319.42		1.543586

				319.44		1.543586

				319.46		1.543586

				319.48		1.543586

				319.5		1.543586

				319.52		1.543586

				319.55		1.539524

				319.57		1.543586

				319.59		1.543586

				319.61		1.543586

				319.63		1.543586

				319.65		1.543586

				319.67		1.543586

				319.69		1.543586

				319.72		1.539524

				319.74		1.543586

				319.76		1.543586

				319.78		1.543586

				319.8		1.539524

				319.82		1.543586

				319.84		1.539524

				319.86		1.539524

				319.88		1.543586

				319.91		1.543586

				319.93		1.543586

				319.95		1.543586

				319.97		1.539524

				319.99		1.539524

				320.01		1.539524

				320.03		1.539524

				320.05		1.539524

				320.07		1.539524

				320.1		1.539524

				320.12		1.539524

				320.14		1.539524

				320.16		1.539524

				320.18		1.539524

				320.2		1.539524

				320.22		1.539524

				320.24		1.539524

				320.27		1.539524

				320.29		1.543586

				320.31		1.539524

				320.33		1.539524

				320.35		1.539524

				320.37		1.539524

				320.39		1.539524

				320.41		1.539524

				320.43		1.539524

				320.46		1.539524

				320.48		1.539524

				320.5		1.539524

				320.52		1.539524

				320.54		1.539524

				320.56		1.539524

				320.58		1.539524

				320.6		1.539524

				320.62		1.539524

				320.65		1.539524

				320.67		1.539524

				320.69		1.539524

				320.71		1.539524

				320.73		1.539524

				320.75		1.539524

				320.77		1.539524

				320.79		1.539524

				320.81		1.539524

				320.84		1.539524

				320.86		1.539524

				320.88		1.539524

				320.9		1.539524

				320.92		1.539524

				320.94		1.539524

				320.96		1.539524

				320.98		1.539524

				321.01		1.539524

				321.03		1.539524

				321.05		1.539524

				321.07		1.539524

				321.09		1.539524

				321.11		1.539524

				321.13		1.539524

				321.15		1.539524

				321.17		1.539524

				321.2		1.539524

				321.22		1.539524

				321.24		1.539524

				321.26		1.539524

				321.28		1.539524

				321.3		1.539524

				321.32		1.539524

				321.34		1.539524

				321.36		1.539524

				321.39		1.539524

				321.41		1.539524

				321.43		1.539524

				321.45		1.539524

				321.47		1.539524

				321.49		1.539524

				321.51		1.539524

				321.53		1.539524

				321.55		1.539524

				321.58		1.539524

				321.6		1.535462

				321.62		1.535462

				321.64		1.535462

				321.66		1.535462

				321.68		1.535462

				321.7		1.535462

				321.72		1.535462

				321.75		1.535462

				321.77		1.535462

				321.79		1.535462

				321.81		1.535462

				321.83		1.535462

				321.85		1.5314

				321.87		1.5314

				321.89		1.5314

				321.91		1.5314

				321.94		1.5314

				321.96		1.5314

				321.98		1.5314

				322		1.5314

				322.02		1.5314

				322.04		1.5314

				322.06		1.527338

				322.08		1.527338

				322.1		1.527338

				322.13		1.5314

				322.15		1.5314

				322.17		1.527338

				322.19		1.527338

				322.21		1.527338

				322.23		1.527338

				322.25		1.527338

				322.27		1.527338

				322.3		1.527338

				322.32		1.527338

				322.34		1.527338

				322.36		1.527338

				322.38		1.527338

				322.4		1.527338

				322.42		1.523276

				322.44		1.523276

				322.46		1.523276

				322.49		1.523276

				322.51		1.527338

				322.53		1.523276

				322.55		1.523276

				322.57		1.523276

				322.59		1.523276

				322.61		1.523276

				322.63		1.523276

				322.66		1.523276

				322.68		1.523276

				322.7		1.523276

				322.72		1.523276

				322.74		1.523276

				322.76		1.523276

				322.78		1.519214

				322.8		1.519214

				322.82		1.519214

				322.85		1.523276

				322.87		1.519214

				322.89		1.523276

				322.91		1.523276

				322.93		1.519214

				322.95		1.523276

				322.97		1.519214

				322.99		1.519214

				323.02		1.519214

				323.04		1.519214

				323.06		1.519214

				323.08		1.519214

				323.1		1.519214

				323.12		1.519214

				323.14		1.519214

				323.16		1.519214

				323.18		1.519214

				323.21		1.519214

				323.23		1.519214

				323.25		1.519214

				323.27		1.519214

				323.29		1.519214

				323.31		1.519214

				323.33		1.519214

				323.35		1.519214

				323.37		1.519214

				323.4		1.519214

				323.42		1.519214

				323.44		1.519214

				323.46		1.519214

				323.48		1.519214

				323.5		1.519214

				323.52		1.519214

				323.54		1.519214

				323.57		1.519214

				323.59		1.515152

				323.61		1.515152

				323.63		1.515152

				323.65		1.515152

				323.67		1.515152

				323.69		1.515152

				323.71		1.515152

				323.73		1.515152

				323.76		1.515152

				323.78		1.515152

				323.8		1.515152

				323.82		1.515152

				323.84		1.515152

				323.86		1.515152

				323.88		1.515152

				323.9		1.515152

				323.93		1.515152

				323.95		1.515152

				323.97		1.515152

				323.99		1.515152

				324.01		1.515152

				324.03		1.515152

				324.05		1.515152

				324.07		1.515152

				324.09		1.515152

				324.12		1.515152

				324.14		1.515152

				324.16		1.515152

				324.18		1.515152

				324.2		1.515152

				324.22		1.515152

				324.24		1.515152

				324.26		1.515152

				324.29		1.515152

				324.31		1.515152

				324.33		1.515152

				324.35		1.515152

				324.37		1.515152

				324.39		1.515152

				324.41		1.515152

				324.43		1.515152

				324.45		1.515152

				324.48		1.515152

				324.5		1.515152

				324.52		1.515152

				324.54		1.515152

				324.56		1.515152

				324.58		1.515152

				324.6		1.515152

				324.62		1.515152

				324.65		1.515152

				324.67		1.515152

				324.69		1.511089

				324.71		1.515152

				324.73		1.511089

				324.75		1.511089

				324.77		1.511089

				324.79		1.511089

				324.81		1.511089

				324.84		1.511089

				324.86		1.511089

				324.88		1.511089

				324.9		1.511089

				324.92		1.511089

				324.94		1.511089

				324.96		1.511089

				324.98		1.511089

				325		1.511089

				325.03		1.511089

				325.05		1.511089

				325.07		1.511089

				325.09		1.511089

				325.11		1.511089

				325.13		1.511089

				325.15		1.511089

				325.17		1.511089

				325.2		1.511089

				325.22		1.511089

				325.24		1.511089

				325.26		1.511089

				325.28		1.511089

				325.3		1.511089

				325.32		1.511089

				325.34		1.511089

				325.36		1.511089

				325.39		1.511089

				325.41		1.511089

				325.43		1.511089

				325.45		1.511089

				325.47		1.511089

				325.49		1.511089

				325.51		1.511089

				325.53		1.511089

				325.56		1.511089

				325.58		1.511089

				325.6		1.511089

				325.62		1.511089

				325.64		1.511089

				325.66		1.511089

				325.68		1.511089

				325.7		1.511089

				325.73		1.515152

				325.75		1.511089

				325.77		1.511089

				325.79		1.515152

				325.81		1.511089

				325.83		1.515152

				325.85		1.515152

				325.87		1.515152

				325.89		1.515152

				325.92		1.515152

				325.94		1.515152

				325.96		1.515152

				325.98		1.515152

				326		1.515152

				326.02		1.515152

				326.04		1.515152

				326.06		1.511089

				326.09		1.515152

				326.11		1.511089

				326.13		1.511089

				326.15		1.511089

				326.17		1.515152

				326.19		1.511089

				326.21		1.511089

				326.23		1.511089

				326.25		1.511089

				326.28		1.511089

				326.3		1.515152

				326.32		1.511089

				326.34		1.511089

				326.36		1.511089

				326.38		1.511089

				326.4		1.511089

				326.42		1.511089

				326.45		1.511089

				326.47		1.511089

				326.49		1.511089

				326.51		1.511089

				326.53		1.511089

				326.55		1.511089

				326.57		1.511089

				326.59		1.511089

				326.62		1.511089

				326.64		1.511089

				326.66		1.511089

				326.68		1.511089

				326.7		1.511089

				326.72		1.511089

				326.74		1.511089

				326.76		1.511089

				326.78		1.511089

				326.81		1.511089

				326.83		1.511089

				326.85		1.511089

				326.87		1.511089

				326.89		1.511089

				326.91		1.511089

				326.93		1.511089

				326.95		1.511089

				326.98		1.511089

				327		1.511089

				327.02		1.511089

				327.04		1.511089

				327.06		1.511089

				327.08		1.511089

				327.1		1.511089

				327.12		1.511089

				327.14		1.511089

				327.17		1.511089

				327.19		1.511089

				327.21		1.511089

				327.23		1.511089

				327.25		1.511089

				327.27		1.511089

				327.29		1.511089

				327.31		1.511089

				327.34		1.515152

				327.36		1.515152

				327.38		1.515152

				327.4		1.515152

				327.42		1.511089

				327.44		1.515152

				327.46		1.511089

				327.48		1.511089

				327.5		1.515152

				327.53		1.511089

				327.55		1.511089

				327.57		1.511089

				327.59		1.511089

				327.61		1.511089

				327.63		1.511089

				327.65		1.515152

				327.67		1.511089

				327.69		1.515152

				327.72		1.515152

				327.74		1.511089

				327.76		1.511089

				327.78		1.515152

				327.8		1.515152

				327.82		1.511089

				327.84		1.515152

				327.86		1.515152

				327.89		1.515152

				327.91		1.515152

				327.93		1.515152

				327.95		1.515152

				327.97		1.515152

				327.99		1.515152

				328.01		1.515152

				328.03		1.515152

				328.05		1.515152

				328.08		1.515152

				328.1		1.515152

				328.12		1.515152

				328.14		1.515152

				328.16		1.515152

				328.18		1.515152

				328.2		1.515152

				328.22		1.515152

				328.25		1.515152

				328.27		1.515152

				328.29		1.515152

				328.31		1.515152

				328.33		1.515152

				328.35		1.515152

				328.37		1.515152

				328.39		1.515152

				328.41		1.515152

				328.44		1.515152

				328.46		1.515152

				328.48		1.515152

				328.5		1.515152

				328.52		1.515152

				328.54		1.515152

				328.56		1.515152

				328.58		1.515152

				328.6		1.515152

				328.63		1.515152

				328.65		1.515152

				328.67		1.515152

				328.69		1.515152

				328.71		1.515152

				328.73		1.515152

				328.75		1.515152

				328.77		1.515152

				328.8		1.515152

				328.82		1.515152

				328.84		1.515152

				328.86		1.515152

				328.88		1.515152

				328.9		1.515152

				328.92		1.515152

				328.94		1.515152

				328.96		1.515152

				328.99		1.515152

				329.01		1.515152

				329.03		1.515152

				329.05		1.515152

				329.07		1.515152

				329.09		1.515152

				329.11		1.515152

				329.13		1.515152

				329.15		1.515152

				329.18		1.515152

				329.2		1.515152

				329.22		1.515152

				329.24		1.515152

				329.26		1.515152

				329.28		1.515152

				329.3		1.515152

				329.32		1.515152

				329.34		1.515152

				329.37		1.515152

				329.39		1.515152

				329.41		1.515152

				329.43		1.515152

				329.45		1.515152

				329.47		1.515152

				329.49		1.515152

				329.51		1.515152

				329.53		1.515152

				329.56		1.515152

				329.58		1.515152

				329.6		1.515152

				329.62		1.515152

				329.64		1.515152

				329.66		1.515152

				329.68		1.515152

				329.7		1.515152

				329.73		1.515152

				329.75		1.515152

				329.77		1.515152

				329.79		1.511089

				329.81		1.515152

				329.83		1.515152

				329.85		1.515152

				329.87		1.515152

				329.89		1.511089

				329.92		1.511089

				329.94		1.515152

				329.96		1.515152

				329.98		1.511089

				330		1.511089

				330.02		1.511089

				330.04		1.511089

				330.06		1.511089

				330.08		1.511089

				330.11		1.511089

				330.13		1.511089

				330.15		1.511089

				330.17		1.511089

				330.19		1.511089

				330.21		1.511089

				330.23		1.511089

				330.25		1.511089

				330.27		1.511089

				330.3		1.511089

				330.32		1.511089

				330.34		1.511089

				330.36		1.511089

				330.38		1.511089

				330.4		1.511089

				330.42		1.511089

				330.44		1.511089

				330.47		1.511089

				330.49		1.511089

				330.51		1.511089

				330.53		1.511089

				330.55		1.511089

				330.57		1.511089

				330.59		1.511089

				330.61		1.511089

				330.63		1.511089

				330.66		1.511089

				330.68		1.511089

				330.7		1.511089

				330.72		1.511089

				330.74		1.511089

				330.76		1.511089

				330.78		1.511089

				330.8		1.511089

				330.82		1.511089

				330.85		1.511089

				330.87		1.511089

				330.89		1.511089

				330.91		1.511089

				330.93		1.511089

				330.95		1.511089

				330.97		1.511089

				330.99		1.511089

				331.01		1.511089

				331.04		1.511089

				331.06		1.511089

				331.08		1.511089

				331.1		1.511089

				331.12		1.511089

				331.14		1.511089

				331.16		1.511089

				331.18		1.511089

				331.2		1.511089

				331.23		1.511089

				331.25		1.511089

				331.27		1.511089

				331.29		1.511089

				331.31		1.511089

				331.33		1.511089

				331.35		1.511089

				331.37		1.511089

				331.39		1.511089

				331.42		1.511089

				331.44		1.511089

				331.46		1.511089

				331.48		1.511089

				331.5		1.511089

				331.52		1.511089

				331.54		1.511089

				331.56		1.511089

				331.58		1.511089

				331.61		1.511089

				331.63		1.511089

				331.65		1.511089

				331.67		1.511089

				331.69		1.511089

				331.71		1.511089

				331.73		1.511089

				331.75		1.511089

				331.77		1.511089

				331.8		1.511089

				331.82		1.511089

				331.84		1.511089

				331.86		1.511089

				331.88		1.511089

				331.9		1.511089

				331.92		1.511089

				331.94		1.511089

				331.96		1.511089

				331.99		1.511089

				332.01		1.511089

				332.03		1.511089

				332.05		1.511089

				332.07		1.511089

				332.09		1.511089

				332.11		1.511089

				332.13		1.511089

				332.15		1.511089

				332.18		1.511089

				332.2		1.511089

				332.22		1.511089

				332.24		1.511089

				332.26		1.511089

				332.28		1.511089

				332.3		1.511089

				332.32		1.511089

				332.35		1.511089

				332.37		1.511089

				332.39		1.511089

				332.41		1.511089

				332.43		1.511089

				332.45		1.511089

				332.47		1.511089

				332.49		1.511089

				332.51		1.511089

				332.54		1.511089

				332.56		1.511089

				332.58		1.511089

				332.6		1.511089

				332.62		1.511089

				332.64		1.511089

				332.66		1.507027

				332.68		1.511089

				332.7		1.511089

				332.73		1.511089

				332.75		1.511089

				332.77		1.511089

				332.79		1.511089

				332.81		1.511089

				332.83		1.511089

				332.85		1.511089

				332.87		1.511089

				332.89		1.511089

				332.92		1.507027

				332.94		1.511089

				332.96		1.507027

				332.98		1.507027

				333		1.507027

				333.02		1.507027

				333.04		1.507027

				333.06		1.507027

				333.08		1.507027

				333.11		1.507027

				333.13		1.507027

				333.15		1.507027

				333.17		1.507027

				333.19		1.507027

				333.21		1.507027

				333.23		1.507027

				333.25		1.507027

				333.27		1.507027

				333.3		1.507027

				333.32		1.507027

				333.34		1.507027

				333.36		1.507027

				333.38		1.507027

				333.4		1.507027

				333.42		1.507027

				333.44		1.507027

				333.46		1.507027

				333.49		1.507027

				333.51		1.507027

				333.53		1.507027

				333.55		1.507027

				333.57		1.507027

				333.59		1.507027

				333.61		1.507027

				333.63		1.507027

				333.66		1.507027

				333.68		1.507027

				333.7		1.507027

				333.72		1.507027

				333.74		1.502965

				333.76		1.502965

				333.78		1.502965

				333.8		1.502965

				333.82		1.502965

				333.85		1.502965

				333.87		1.502965

				333.89		1.502965

				333.91		1.502965

				333.93		1.502965

				333.95		1.502965

				333.97		1.502965

				333.99		1.502965

				334.01		1.502965

				334.04		1.502965

				334.06		1.502965

				334.08		1.502965

				334.1		1.502965

				334.12		1.502965

				334.14		1.502965

				334.16		1.502965

				334.18		1.502965

				334.2		1.502965

				334.23		1.502965

				334.25		1.502965

				334.27		1.502965

				334.29		1.502965

				334.31		1.502965

				334.33		1.498903

				334.35		1.502965

				334.37		1.498903

				334.39		1.498903

				334.42		1.498903

				334.44		1.498903

				334.46		1.498903

				334.48		1.498903

				334.5		1.498903

				334.52		1.498903

				334.54		1.498903

				334.56		1.498903

				334.58		1.498903

				334.61		1.498903

				334.63		1.498903

				334.65		1.498903

				334.67		1.498903

				334.69		1.498903

				334.71		1.498903

				334.73		1.498903

				334.75		1.498903

				334.77		1.498903

				334.8		1.498903

				334.82		1.494841

				334.84		1.494841

				334.86		1.494841

				334.88		1.494841

				334.9		1.494841

				334.92		1.494841

				334.94		1.494841

				334.96		1.494841

				334.99		1.494841

				335.01		1.494841

				335.03		1.494841

				335.05		1.494841

				335.07		1.494841

				335.09		1.494841

				335.11		1.494841

				335.13		1.494841

				335.15		1.494841

				335.18		1.490779

				335.2		1.494841

				335.22		1.490779

				335.24		1.490779

				335.26		1.490779

				335.28		1.490779

				335.3		1.490779

				335.32		1.490779

				335.34		1.490779

				335.37		1.490779

				335.39		1.490779

				335.41		1.490779

				335.43		1.490779

				335.45		1.490779

				335.47		1.490779

				335.49		1.490779

				335.51		1.490779

				335.53		1.490779

				335.56		1.490779

				335.58		1.490779

				335.6		1.490779

				335.62		1.490779

				335.64		1.490779

				335.66		1.490779

				335.68		1.490779

				335.7		1.490779

				335.72		1.486717

				335.75		1.486717

				335.77		1.486717

				335.79		1.486717

				335.81		1.486717

				335.83		1.486717

				335.85		1.486717

				335.87		1.486717

				335.89		1.486717

				335.92		1.486717

				335.94		1.486717

				335.96		1.486717

				335.98		1.486717

				336		1.486717

				336.02		1.486717

				336.04		1.486717

				336.06		1.486717

				336.08		1.486717

				336.11		1.486717

				336.13		1.482655

				336.15		1.482655

				336.17		1.482655

				336.19		1.482655

				336.21		1.482655

				336.23		1.482655

				336.25		1.482655

				336.27		1.482655

				336.3		1.482655

				336.32		1.482655

				336.34		1.482655

				336.36		1.482655

				336.38		1.482655

				336.4		1.482655

				336.42		1.482655

				336.44		1.478593

				336.46		1.482655

				336.49		1.482655

				336.51		1.478593

				336.53		1.478593

				336.55		1.482655

				336.57		1.478593

				336.59		1.478593

				336.61		1.482655

				336.63		1.478593

				336.65		1.482655

				336.68		1.478593

				336.7		1.478593

				336.72		1.478593

				336.74		1.478593

				336.76		1.478593

				336.78		1.478593

				336.8		1.478593

				336.82		1.478593

				336.84		1.478593

				336.87		1.478593

				336.89		1.478593

				336.91		1.478593

				336.93		1.478593

				336.95		1.478593

				336.97		1.478593

				336.99		1.478593

				337.01		1.478593

				337.04		1.478593

				337.06		1.478593

				337.08		1.478593

				337.1		1.478593

				337.12		1.478593

				337.14		1.478593

				337.16		1.478593

				337.18		1.478593

				337.2		1.478593

				337.23		1.478593

				337.25		1.478593

				337.27		1.478593

				337.29		1.478593

				337.31		1.478593

				337.33		1.478593

				337.35		1.478593

				337.37		1.478593

				337.39		1.478593

				337.42		1.478593

				337.44		1.478593

				337.46		1.478593

				337.48		1.478593

				337.5		1.478593

				337.52		1.478593

				337.54		1.478593

				337.56		1.478593

				337.58		1.478593

				337.61		1.478593

				337.63		1.478593

				337.65		1.478593

				337.67		1.478593

				337.69		1.478593

				337.71		1.478593

				337.73		1.478593

				337.75		1.478593

				337.77		1.478593

				337.8		1.474531

				337.82		1.478593

				337.84		1.478593

				337.86		1.478593

				337.88		1.478593

				337.9		1.478593

				337.92		1.478593

				337.94		1.478593

				337.96		1.478593

				337.99		1.478593

				338.01		1.478593

				338.03		1.478593

				338.05		1.478593

				338.07		1.478593

				338.09		1.478593

				338.11		1.478593

				338.13		1.478593

				338.15		1.478593

				338.18		1.478593

				338.2		1.478593

				338.22		1.478593

				338.24		1.478593

				338.26		1.478593

				338.28		1.478593

				338.3		1.478593

				338.32		1.478593

				338.35		1.478593

				338.37		1.478593

				338.39		1.478593

				338.41		1.478593

				338.43		1.478593

				338.45		1.478593

				338.47		1.478593

				338.49		1.478593

				338.51		1.478593

				338.54		1.478593

				338.56		1.482655

				338.58		1.482655

				338.6		1.478593

				338.62		1.482655

				338.64		1.478593

				338.66		1.478593

				338.68		1.478593

				338.7		1.478593

				338.73		1.478593

				338.75		1.478593

				338.77		1.478593

				338.79		1.478593

				338.81		1.478593

				338.83		1.478593

				338.85		1.478593

				338.87		1.478593

				338.89		1.478593

				338.92		1.478593

				338.94		1.478593

				338.96		1.478593

				338.98		1.478593

				339		1.478593

				339.02		1.478593

				339.04		1.478593

				339.06		1.478593

				339.08		1.478593

				339.11		1.478593

				339.13		1.478593

				339.15		1.478593

				339.17		1.478593

				339.19		1.478593

				339.21		1.478593

				339.23		1.478593

				339.25		1.478593

				339.27		1.478593

				339.3		1.478593

				339.32		1.482655

				339.34		1.478593

				339.36		1.478593

				339.38		1.478593

				339.4		1.478593

				339.42		1.478593

				339.44		1.478593

				339.47		1.478593

				339.49		1.478593

				339.51		1.478593

				339.53		1.478593

				339.55		1.478593

				339.57		1.478593

				339.59		1.478593

				339.61		1.478593

				339.63		1.478593

				339.66		1.478593

				339.68		1.478593

				339.7		1.478593

				339.72		1.478593

				339.74		1.478593

				339.76		1.478593

				339.78		1.478593

				339.8		1.478593

				339.83		1.478593

				339.85		1.478593

				339.87		1.478593

				339.89		1.478593

				339.91		1.478593

				339.93		1.478593

				339.95		1.478593

				339.97		1.478593

				339.99		1.478593

				340.02		1.478593

				340.04		1.478593

				340.06		1.478593

				340.08		1.474531

				340.1		1.474531

				340.12		1.474531

				340.14		1.474531

				340.16		1.474531

				340.18		1.474531

				340.21		1.474531

				340.23		1.474531

				340.25		1.474531

				340.27		1.474531

				340.29		1.474531

				340.31		1.474531

				340.33		1.474531

				340.35		1.474531

				340.37		1.474531

				340.4		1.474531

				340.42		1.474531

				340.44		1.474531

				340.46		1.470469

				340.48		1.470469

				340.5		1.470469

				340.52		1.470469

				340.54		1.470469

				340.57		1.470469

				340.59		1.470469

				340.61		1.470469

				340.63		1.470469

				340.65		1.470469

				340.67		1.470469

				340.69		1.470469

				340.71		1.470469

				340.73		1.470469

				340.76		1.470469

				340.78		1.470469

				340.8		1.470469

				340.82		1.470469

				340.84		1.470469

				340.86		1.470469

				340.88		1.470469

				340.9		1.470469

				340.92		1.470469

				340.95		1.470469

				340.97		1.470469

				340.99		1.470469

				341.01		1.470469

				341.03		1.470469

				341.05		1.470469

				341.07		1.470469

				341.09		1.470469

				341.11		1.470469

				341.14		1.470469

				341.16		1.470469

				341.18		1.470469

				341.2		1.470469

				341.22		1.470469

				341.24		1.466407

				341.26		1.466407

				341.28		1.466407

				341.3		1.466407

				341.33		1.466407

				341.35		1.466407

				341.37		1.466407

				341.39		1.466407

				341.41		1.466407

				341.43		1.466407

				341.45		1.466407

				341.47		1.466407

				341.49		1.466407

				341.52		1.466407

				341.54		1.466407

				341.56		1.462345

				341.58		1.462345

				341.6		1.466407

				341.62		1.462345

				341.64		1.462345

				341.66		1.462345

				341.69		1.462345

				341.71		1.462345

				341.73		1.462345

				341.75		1.462345

				341.77		1.462345

				341.79		1.462345

				341.81		1.462345

				341.83		1.462345

				341.85		1.462345

				341.88		1.462345

				341.9		1.462345

				341.92		1.462345

				341.94		1.462345

				341.96		1.462345

				341.98		1.462345

				342		1.462345

				342.02		1.462345

				342.04		1.462345

				342.07		1.462345

				342.09		1.462345

				342.11		1.462345

				342.13		1.462345

				342.15		1.462345

				342.17		1.462345

				342.19		1.462345

				342.21		1.462345

				342.23		1.462345

				342.26		1.462345

				342.28		1.462345

				342.3		1.462345

				342.32		1.462345

				342.34		1.462345

				342.36		1.462345

				342.38		1.462345

				342.4		1.462345

				342.42		1.462345

				342.45		1.462345

				342.47		1.462345

				342.49		1.462345

				342.51		1.462345

				342.53		1.462345

				342.55		1.462345

				342.57		1.462345

				342.59		1.462345

				342.61		1.462345

				342.64		1.462345

				342.66		1.462345

				342.68		1.462345

				342.7		1.462345

				342.72		1.458283

				342.74		1.458283

				342.76		1.462345

				342.78		1.458283

				342.8		1.458283

				342.83		1.458283

				342.85		1.458283

				342.87		1.458283

				342.89		1.458283

				342.91		1.458283

				342.93		1.458283

				342.95		1.458283

				342.97		1.458283

				342.99		1.458283

				343.02		1.458283

				343.04		1.458283

				343.06		1.45422

				343.08		1.458283

				343.1		1.458283

				343.12		1.458283

				343.14		1.458283

				343.16		1.458283

				343.18		1.458283

				343.21		1.45422

				343.23		1.458283

				343.25		1.45422

				343.27		1.45422

				343.29		1.45422

				343.31		1.45422

				343.33		1.45422

				343.35		1.45422

				343.38		1.45422

				343.4		1.45422

				343.42		1.45422

				343.44		1.45422

				343.46		1.45422

				343.48		1.45422

				343.5		1.45422

				343.52		1.45422

				343.54		1.45422

				343.57		1.450158

				343.59		1.450158

				343.61		1.450158

				343.63		1.450158

				343.65		1.450158

				343.67		1.450158

				343.69		1.450158

				343.71		1.450158

				343.73		1.450158

				343.76		1.450158

				343.78		1.450158

				343.8		1.45422

				343.82		1.45422

				343.84		1.45422

				343.86		1.45422

				343.88		1.45422

				343.9		1.45422

				343.92		1.45422

				343.95		1.45422

				343.97		1.45422

				343.99		1.45422

				344.01		1.450158

				344.03		1.450158

				344.05		1.450158

				344.07		1.45422

				344.09		1.450158

				344.11		1.450158

				344.14		1.450158

				344.16		1.450158

				344.18		1.450158

				344.2		1.450158

				344.22		1.450158

				344.24		1.450158

				344.26		1.450158

				344.28		1.450158

				344.3		1.450158

				344.33		1.450158

				344.35		1.450158

				344.37		1.450158

				344.39		1.450158

				344.41		1.450158

				344.43		1.450158

				344.45		1.450158

				344.47		1.450158

				344.49		1.450158

				344.52		1.450158

				344.54		1.450158

				344.56		1.450158

				344.58		1.450158

				344.6		1.450158

				344.62		1.450158

				344.64		1.450158

				344.66		1.450158

				344.68		1.450158

				344.71		1.450158

				344.73		1.446096

				344.75		1.446096

				344.77		1.446096

				344.79		1.446096

				344.81		1.446096

				344.83		1.446096

				344.85		1.446096

				344.87		1.446096

				344.9		1.446096

				344.92		1.446096

				344.94		1.450158

				344.96		1.450158

				344.98		1.450158

				345		1.450158

				345.02		1.450158

				345.04		1.450158

				345.06		1.446096

				345.09		1.450158

				345.11		1.446096

				345.13		1.450158

				345.15		1.450158

				345.17		1.450158

				345.19		1.450158

				345.21		1.450158

				345.23		1.446096

				345.25		1.446096

				345.27		1.446096

				345.3		1.446096

				345.32		1.446096

				345.34		1.446096

				345.36		1.446096

				345.38		1.446096

				345.4		1.446096

				345.42		1.446096

				345.44		1.446096

				345.46		1.446096

				345.49		1.446096

				345.51		1.446096

				345.53		1.446096

				345.55		1.446096

				345.57		1.446096

				345.59		1.446096

				345.61		1.446096

				345.63		1.446096

				345.65		1.446096

				345.68		1.446096

				345.7		1.446096

				345.72		1.446096

				345.74		1.446096

				345.76		1.446096

				345.78		1.446096

				345.8		1.446096

				345.82		1.446096

				345.84		1.446096

				345.86		1.446096

				345.89		1.446096

				345.91		1.446096

				345.93		1.446096

				345.95		1.446096

				345.97		1.446096

				345.99		1.446096

				346.01		1.446096

				346.03		1.446096

				346.05		1.446096

				346.08		1.446096

				346.1		1.446096

				346.12		1.446096

				346.14		1.446096

				346.16		1.446096

				346.18		1.446096

				346.2		1.442034

				346.22		1.446096

				346.24		1.446096

				346.27		1.442034

				346.29		1.446096

				346.31		1.446096

				346.33		1.446096

				346.35		1.446096

				346.37		1.446096

				346.39		1.446096

				346.41		1.442034

				346.43		1.446096

				346.45		1.442034

				346.48		1.442034

				346.5		1.446096

				346.52		1.442034

				346.54		1.442034

				346.56		1.442034

				346.58		1.442034

				346.6		1.442034

				346.62		1.442034

				346.64		1.442034

				346.67		1.442034

				346.69		1.442034

				346.71		1.442034

				346.73		1.442034

				346.75		1.442034

				346.77		1.442034

				346.79		1.442034

				346.81		1.442034

				346.83		1.442034

				346.86		1.442034

				346.88		1.442034

				346.9		1.442034

				346.92		1.442034

				346.94		1.442034

				346.96		1.442034

				346.98		1.442034

				347		1.442034

				347.02		1.442034

				347.05		1.437972

				347.07		1.442034

				347.09		1.442034

				347.11		1.437972

				347.13		1.437972

				347.15		1.437972

				347.17		1.437972

				347.19		1.437972

				347.21		1.437972

				347.23		1.437972

				347.26		1.437972

				347.28		1.437972

				347.3		1.437972

				347.32		1.437972

				347.34		1.437972

				347.36		1.437972

				347.38		1.437972

				347.4		1.437972

				347.42		1.437972

				347.45		1.437972

				347.47		1.437972

				347.49		1.437972

				347.51		1.437972

				347.53		1.437972

				347.55		1.43391

				347.57		1.437972

				347.59		1.437972

				347.61		1.43391

				347.63		1.437972

				347.66		1.43391

				347.68		1.43391

				347.7		1.43391

				347.72		1.43391

				347.74		1.43391

				347.76		1.43391

				347.78		1.43391

				347.8		1.43391

				347.82		1.43391

				347.85		1.43391

				347.87		1.43391

				347.89		1.43391

				347.91		1.43391

				347.93		1.43391

				347.95		1.43391

				347.97		1.43391

				347.99		1.43391

				348.01		1.43391

				348.03		1.43391

				348.06		1.43391

				348.08		1.43391

				348.1		1.43391

				348.12		1.43391

				348.14		1.43391

				348.16		1.43391

				348.18		1.43391

				348.2		1.43391

				348.22		1.43391

				348.25		1.43391

				348.27		1.429848

				348.29		1.43391

				348.31		1.43391

				348.33		1.429848

				348.35		1.43391

				348.37		1.429848

				348.39		1.429848

				348.41		1.429848

				348.43		1.429848

				348.46		1.429848

				348.48		1.429848

				348.5		1.429848

				348.52		1.429848

				348.54		1.429848

				348.56		1.429848

				348.58		1.429848

				348.6		1.429848

				348.62		1.429848

				348.65		1.429848

				348.67		1.429848

				348.69		1.429848

				348.71		1.429848

				348.73		1.429848

				348.75		1.429848

				348.77		1.429848

				348.79		1.429848

				348.81		1.429848

				348.84		1.429848

				348.86		1.429848

				348.88		1.429848

				348.9		1.429848

				348.92		1.429848

				348.94		1.429848

				348.96		1.429848

				348.98		1.429848

				349		1.429848

				349.02		1.429848

				349.05		1.429848

				349.07		1.429848

				349.09		1.429848

				349.11		1.425786

				349.13		1.429848

				349.15		1.425786

				349.17		1.425786

				349.19		1.429848

				349.22		1.425786

				349.24		1.429848

				349.26		1.429848

				349.28		1.425786

				349.3		1.429848

				349.32		1.429848

				349.34		1.429848

				349.36		1.425786

				349.38		1.425786

				349.41		1.425786

				349.43		1.425786

				349.45		1.425786

				349.47		1.425786

				349.49		1.425786

				349.51		1.425786

				349.53		1.425786

				349.56		1.425786

				349.58		1.425786

				349.6		1.425786

				349.62		1.425786

				349.64		1.425786

				349.66		1.425786

				349.68		1.425786

				349.7		1.425786

				349.73		1.425786

				349.75		1.425786

				349.77		1.425786

				349.79		1.425786

				349.81		1.425786

				349.83		1.425786

				349.85		1.425786

				349.88		1.425786

				349.9		1.425786

				349.92		1.425786

				349.94		1.425786

				349.96		1.425786

				349.98		1.425786

				350		1.425786

				350.02		1.425786

				350.05		1.425786

				350.07		1.425786

				350.09		1.425786

				350.11		1.425786

				350.13		1.425786

				350.15		1.425786

				350.17		1.425786

				350.19		1.425786

				350.22		1.425786

				350.24		1.425786

				350.26		1.425786

				350.28		1.421724

				350.3		1.421724

				350.32		1.421724

				350.34		1.421724

				350.36		1.421724

				350.38		1.421724

				350.41		1.421724

				350.43		1.421724

				350.45		1.421724

				350.47		1.421724

				350.49		1.421724

				350.51		1.421724

				350.53		1.421724

				350.55		1.421724

				350.58		1.421724

				350.6		1.421724

				350.62		1.421724

				350.64		1.421724

				350.66		1.421724

				350.68		1.421724

				350.7		1.421724

				350.72		1.421724

				350.74		1.421724

				350.77		1.417662

				350.79		1.417662

				350.81		1.417662

				350.83		1.417662

				350.85		1.417662

				350.87		1.417662

				350.89		1.417662

				350.91		1.417662

				350.93		1.417662

				350.96		1.417662

				350.98		1.417662

				351		1.417662

				351.02		1.417662

				351.04		1.417662

				351.06		1.417662

				351.08		1.417662

				351.1		1.417662

				351.12		1.417662

				351.15		1.417662

				351.17		1.417662

				351.19		1.417662

				351.21		1.417662

				351.23		1.417662

				351.25		1.417662

				351.27		1.417662

				351.29		1.417662

				351.31		1.417662

				351.34		1.417662

				351.36		1.417662

				351.38		1.417662

				351.4		1.417662

				351.42		1.417662

				351.44		1.417662

				351.46		1.417662

				351.48		1.417662

				351.51		1.417662

				351.53		1.417662

				351.55		1.417662

				351.57		1.417662

				351.59		1.4136

				351.61		1.4136

				351.63		1.4136

				351.65		1.4136

				351.67		1.4136

				351.7		1.4136

				351.72		1.4136

				351.74		1.4136

				351.76		1.4136

				351.78		1.4136

				351.8		1.4136

				351.82		1.4136

				351.84		1.4136

				351.87		1.4136

				351.89		1.4136

				351.91		1.4136

				351.93		1.4136

				351.95		1.4136

				351.97		1.4136

				351.99		1.4136

				352.01		1.4136

				352.03		1.4136

				352.06		1.4136

				352.08		1.4136

				352.1		1.4136

				352.12		1.4136

				352.14		1.4136

				352.16		1.4136

				352.18		1.4136

				352.2		1.4136

				352.23		1.4136

				352.25		1.4136

				352.27		1.4136

				352.29		1.4136

				352.31		1.4136

				352.33		1.4136

				352.35		1.4136

				352.37		1.4136

				352.39		1.4136

				352.42		1.4136

				352.44		1.4136

				352.46		1.4136

				352.48		1.4136

				352.5		1.4136

				352.52		1.4136

				352.54		1.4136

				352.56		1.4136

				352.59		1.4136

				352.61		1.4136

				352.63		1.4136

				352.65		1.4136

				352.67		1.4136

				352.69		1.4136

				352.71		1.4136

				352.73		1.4136

				352.76		1.4136

				352.78		1.4136

				352.8		1.4136

				352.82		1.4136

				352.84		1.4136

				352.86		1.4136

				352.88		1.4136

				352.9		1.4136

				352.92		1.4136

				352.95		1.409538

				352.97		1.409538

				352.99		1.409538

				353.01		1.409538

				353.03		1.409538

				353.05		1.409538

				353.07		1.409538

				353.09		1.409538

				353.12		1.409538

				353.14		1.409538

				353.16		1.409538

				353.18		1.409538

				353.2		1.409538

				353.22		1.409538

				353.24		1.409538

				353.26		1.409538

				353.28		1.409538

				353.31		1.409538

				353.33		1.409538

				353.35		1.409538

				353.37		1.409538

				353.39		1.409538

				353.41		1.409538

				353.43		1.409538

				353.45		1.405476

				353.48		1.405476

				353.5		1.405476

				353.52		1.405476

				353.54		1.405476

				353.56		1.405476

				353.58		1.405476

				353.6		1.405476

				353.62		1.405476

				353.64		1.405476

				353.67		1.405476

				353.69		1.405476

				353.71		1.405476

				353.73		1.405476

				353.75		1.405476

				353.77		1.405476

				353.79		1.405476

				353.81		1.405476

				353.84		1.405476

				353.86		1.405476

				353.88		1.405476

				353.9		1.405476

				353.92		1.405476

				353.94		1.405476

				353.96		1.401414

				353.98		1.401414

				354		1.401414

				354.03		1.401414

				354.05		1.401414

				354.07		1.401414

				354.09		1.401414

				354.11		1.401414

				354.13		1.401414

				354.15		1.401414

				354.17		1.401414

				354.2		1.401414

				354.22		1.397352

				354.24		1.397352

				354.26		1.397352

				354.28		1.397352

				354.3		1.397352

				354.32		1.397352

				354.34		1.397352

				354.37		1.397352

				354.39		1.397352

				354.41		1.393289

				354.43		1.393289

				354.45		1.393289

				354.47		1.393289

				354.49		1.393289

				354.51		1.393289

				354.53		1.393289

				354.56		1.393289

				354.58		1.393289

				354.6		1.393289

				354.62		1.393289

				354.64		1.393289

				354.66		1.393289

				354.68		1.393289

				354.7		1.393289

				354.73		1.393289

				354.75		1.393289

				354.77		1.393289

				354.79		1.393289

				354.81		1.393289

				354.83		1.393289

				354.85		1.393289

				354.87		1.393289

				354.89		1.389227

				354.92		1.389227

				354.94		1.389227

				354.96		1.389227

				354.98		1.389227

				355		1.389227

				355.02		1.389227

				355.04		1.389227

				355.06		1.389227

				355.09		1.389227

				355.11		1.389227

				355.13		1.389227

				355.15		1.389227

				355.17		1.389227

				355.19		1.389227

				355.21		1.389227

				355.23		1.389227

				355.26		1.389227

				355.28		1.389227

				355.3		1.389227

				355.32		1.389227

				355.34		1.389227

				355.36		1.389227

				355.38		1.389227

				355.4		1.389227

				355.43		1.389227

				355.45		1.389227

				355.47		1.389227

				355.49		1.389227

				355.51		1.389227

				355.53		1.385165

				355.55		1.389227

				355.57		1.389227

				355.6		1.389227

				355.62		1.385165

				355.64		1.385165

				355.66		1.385165

				355.68		1.385165

				355.7		1.385165

				355.72		1.385165

				355.74		1.385165

				355.77		1.385165

				355.79		1.385165

				355.81		1.385165

				355.83		1.385165

				355.85		1.385165

				355.87		1.389227

				355.89		1.389227

				355.91		1.385165

				355.93		1.385165

				355.96		1.389227

				355.98		1.389227

				356		1.389227

				356.02		1.389227

				356.04		1.389227

				356.06		1.389227

				356.08		1.389227

				356.1		1.389227

				356.13		1.389227

				356.15		1.389227

				356.17		1.385165

				356.19		1.389227

				356.21		1.385165

				356.23		1.385165

				356.25		1.385165

				356.27		1.385165

				356.3		1.385165

				356.32		1.385165

				356.34		1.385165

				356.36		1.389227

				356.38		1.389227

				356.4		1.389227

				356.42		1.389227

				356.44		1.389227

				356.47		1.389227

				356.49		1.389227

				356.51		1.389227

				356.53		1.389227

				356.55		1.389227

				356.57		1.389227

				356.59		1.389227

				356.61		1.389227

				356.64		1.389227

				356.66		1.389227

				356.68		1.389227

				356.7		1.389227

				356.72		1.389227

				356.74		1.389227

				356.76		1.389227

				356.78		1.385165

				356.8		1.385165

				356.83		1.385165

				356.85		1.385165

				356.87		1.385165

				356.89		1.385165

				356.91		1.385165

				356.93		1.385165

				356.95		1.385165

				356.97		1.385165

				357		1.385165

				357.02		1.385165

				357.04		1.385165

				357.06		1.385165

				357.08		1.385165

				357.1		1.385165

				357.12		1.385165

				357.14		1.385165

				357.17		1.385165

				357.19		1.385165

				357.21		1.385165

				357.23		1.385165

				357.25		1.385165

				357.27		1.385165

				357.29		1.385165

				357.31		1.385165

				357.34		1.385165

				357.36		1.385165

				357.38		1.385165

				357.4		1.385165

				357.42		1.385165

				357.44		1.385165

				357.46		1.385165

				357.48		1.381103

				357.5		1.385165

				357.53		1.385165

				357.55		1.381103

				357.57		1.381103

				357.59		1.381103

				357.61		1.381103

				357.63		1.381103

				357.65		1.381103

				357.67		1.381103

				357.7		1.381103

				357.72		1.381103

				357.74		1.381103

				357.76		1.381103

				357.78		1.381103

				357.8		1.381103

				357.82		1.381103

				357.84		1.381103

				357.87		1.381103

				357.89		1.381103

				357.91		1.381103

				357.93		1.381103

				357.95		1.381103

				357.97		1.381103

				357.99		1.381103

				358.01		1.381103

				358.04		1.381103

				358.06		1.377041

				358.08		1.377041

				358.1		1.377041

				358.12		1.377041

				358.14		1.377041

				358.16		1.377041

				358.18		1.377041

				358.21		1.377041

				358.23		1.377041

				358.25		1.377041

				358.27		1.377041

				358.29		1.377041

				358.31		1.377041

				358.33		1.377041

				358.35		1.377041

				358.37		1.377041

				358.4		1.377041

				358.42		1.377041

				358.44		1.377041

				358.46		1.377041

				358.48		1.377041

				358.5		1.377041

				358.52		1.377041

				358.54		1.377041

				358.57		1.377041

				358.59		1.377041

				358.61		1.377041

				358.63		1.377041

				358.65		1.377041

				358.67		1.377041

				358.69		1.377041

				358.71		1.377041

				358.74		1.377041

				358.76		1.377041

				358.78		1.377041

				358.8		1.377041

				358.82		1.377041

				358.84		1.377041

				358.86		1.377041

				358.88		1.372979

				358.9		1.377041

				358.93		1.372979

				358.95		1.372979

				358.97		1.372979

				358.99		1.372979

				359.01		1.372979

				359.03		1.372979

				359.05		1.372979

				359.07		1.372979

				359.1		1.372979

				359.12		1.372979

				359.14		1.372979

				359.16		1.372979

				359.18		1.372979

				359.2		1.372979

				359.22		1.372979

				359.24		1.372979

				359.27		1.372979

				359.29		1.372979

				359.31		1.372979

				359.33		1.372979

				359.35		1.372979

				359.37		1.372979

				359.39		1.372979

				359.41		1.372979

				359.44		1.372979

				359.46		1.372979

				359.48		1.372979

				359.5		1.372979

				359.52		1.372979

				359.54		1.372979

				359.56		1.368917

				359.58		1.372979

				359.6		1.372979

				359.63		1.372979

				359.65		1.372979

				359.67		1.372979

				359.69		1.372979

				359.71		1.372979

				359.73		1.372979

				359.75		1.368917

				359.77		1.368917

				359.8		1.368917

				359.82		1.372979

				359.84		1.368917

				359.86		1.368917

				359.88		1.368917

				359.9		1.368917

				359.92		1.368917

				359.94		1.368917

				359.97		1.368917

				359.99		1.368917

				360.01		1.368917

				360.03		1.368917

				360.05		1.368917

				360.07		1.368917

				360.09		1.368917

				360.11		1.368917

				360.13		1.368917

				360.16		1.368917

				360.18		1.368917

				360.2		1.368917

				360.22		1.368917

				360.24		1.368917

				360.26		1.368917

				360.28		1.368917

				360.3		1.368917

				360.33		1.368917

				360.35		1.368917

				360.37		1.364855

				360.39		1.364855

				360.41		1.364855

				360.43		1.364855

				360.45		1.364855

				360.47		1.364855

				360.5		1.364855

				360.52		1.364855

				360.54		1.364855

				360.56		1.364855

				360.58		1.364855

				360.6		1.364855

				360.62		1.364855

				360.64		1.364855

				360.66		1.364855

				360.69		1.364855

				360.71		1.364855

				360.73		1.364855

				360.75		1.364855

				360.77		1.364855

				360.79		1.364855

				360.81		1.364855

				360.83		1.364855

				360.86		1.364855

				360.88		1.364855

				360.9		1.364855

				360.92		1.364855

				360.94		1.364855

				360.96		1.364855

				360.98		1.364855

				361		1.364855

				361.03		1.364855

				361.05		1.364855

				361.07		1.364855

				361.09		1.364855

				361.11		1.364855

				361.13		1.364855

				361.15		1.364855

				361.17		1.364855

				361.2		1.364855

				361.22		1.364855

				361.24		1.364855

				361.26		1.364855

				361.28		1.364855

				361.3		1.364855

				361.32		1.364855

				361.34		1.364855

				361.36		1.364855

				361.39		1.364855

				361.41		1.364855

				361.43		1.364855

				361.45		1.364855

				361.47		1.364855

				361.49		1.364855

				361.51		1.364855

				361.53		1.364855

				361.56		1.364855

				361.58		1.364855

				361.6		1.364855

				361.62		1.364855

				361.64		1.364855

				361.66		1.364855

				361.68		1.364855

				361.7		1.364855

				361.73		1.364855

				361.75		1.364855

				361.77		1.364855

				361.79		1.364855

				361.81		1.364855

				361.83		1.364855

				361.85		1.364855

				361.87		1.364855

				361.9		1.364855

				361.92		1.364855

				361.94		1.364855

				361.96		1.364855

				361.98		1.364855

				362		1.364855

				362.02		1.364855

				362.04		1.364855

				362.06		1.364855

				362.09		1.364855

				362.11		1.364855

				362.13		1.364855

				362.15		1.364855

				362.17		1.364855

				362.19		1.364855

				362.21		1.364855

				362.23		1.364855

				362.26		1.364855

				362.28		1.364855

				362.3		1.364855

				362.32		1.364855

				362.34		1.364855

				362.36		1.364855

				362.38		1.364855

				362.4		1.364855

				362.43		1.364855

				362.45		1.364855

				362.47		1.364855

				362.49		1.364855

				362.51		1.364855

				362.53		1.364855

				362.55		1.368917

				362.57		1.368917

				362.6		1.364855

				362.62		1.364855

				362.64		1.368917

				362.66		1.368917

				362.68		1.368917

				362.7		1.368917

				362.72		1.368917

				362.74		1.368917

				362.76		1.368917

				362.79		1.368917

				362.81		1.368917

				362.83		1.368917

				362.85		1.368917

				362.87		1.368917

				362.89		1.368917

				362.91		1.368917

				362.93		1.368917

				362.96		1.368917

				362.98		1.368917

				363		1.368917

				363.02		1.368917

				363.04		1.368917

				363.06		1.368917

				363.08		1.368917

				363.1		1.368917

				363.13		1.368917

				363.15		1.368917

				363.17		1.368917

				363.19		1.368917

				363.21		1.372979

				363.23		1.372979

				363.25		1.372979

				363.27		1.372979

				363.29		1.372979

				363.32		1.372979

				363.34		1.368917

				363.36		1.372979

				363.38		1.368917

				363.4		1.368917

				363.42		1.368917

				363.44		1.368917

				363.46		1.368917

				363.49		1.368917

				363.51		1.368917

				363.53		1.368917

				363.55		1.368917

				363.57		1.368917

				363.59		1.368917

				363.61		1.368917

				363.63		1.368917

				363.65		1.368917

				363.68		1.368917

				363.7		1.368917

				363.72		1.368917

				363.74		1.368917

				363.76		1.368917

				363.78		1.368917

				363.8		1.368917

				363.82		1.368917

				363.85		1.368917

				363.87		1.368917

				363.89		1.368917

				363.91		1.368917

				363.93		1.368917

				363.95		1.368917

				363.97		1.364855

				363.99		1.368917

				364.02		1.368917

				364.04		1.364855

				364.06		1.364855

				364.08		1.364855

				364.1		1.368917

				364.12		1.364855

				364.14		1.364855

				364.16		1.368917

				364.18		1.368917

				364.21		1.368917

				364.23		1.364855

				364.25		1.368917

				364.27		1.368917

				364.29		1.368917

				364.31		1.368917

				364.33		1.368917

				364.35		1.368917

				364.38		1.368917

				364.4		1.368917

				364.42		1.368917

				364.44		1.368917

				364.46		1.368917

				364.48		1.368917

				364.5		1.368917

				364.52		1.368917

				364.55		1.368917

				364.57		1.368917

				364.59		1.368917

				364.61		1.368917

				364.63		1.368917

				364.65		1.368917

				364.67		1.368917

				364.69		1.368917

				364.71		1.368917

				364.74		1.368917

				364.76		1.364855

				364.78		1.364855

				364.8		1.364855

				364.82		1.364855

				364.84		1.364855

				364.86		1.364855

				364.88		1.364855

				364.91		1.364855

				364.93		1.364855

				364.95		1.364855

				364.97		1.364855

				364.99		1.364855

				365.01		1.364855

				365.03		1.364855

				365.05		1.364855

				365.08		1.364855

				365.1		1.364855

				365.12		1.364855

				365.14		1.364855

				365.16		1.364855

				365.18		1.364855

				365.2		1.364855

				365.22		1.364855

				365.24		1.364855

				365.27		1.364855

				365.29		1.364855

				365.31		1.364855

				365.33		1.364855

				365.35		1.360793

				365.37		1.364855

				365.39		1.364855

				365.41		1.364855

				365.44		1.364855

				365.46		1.364855

				365.48		1.364855

				365.5		1.364855

				365.52		1.364855

				365.54		1.364855

				365.56		1.364855

				365.58		1.364855

				365.61		1.364855

				365.63		1.364855

				365.65		1.364855

				365.67		1.364855

				365.69		1.364855

				365.71		1.364855

				365.73		1.364855

				365.75		1.364855

				365.78		1.364855

				365.8		1.364855

				365.82		1.364855

				365.84		1.364855

				365.86		1.364855

				365.88		1.364855

				365.9		1.364855

				365.92		1.364855

				365.94		1.368917

				365.97		1.368917

				365.99		1.368917

				366.01		1.368917

				366.03		1.368917

				366.05		1.368917

				366.07		1.368917

				366.09		1.368917

				366.11		1.368917

				366.14		1.368917

				366.16		1.368917

				366.18		1.368917

				366.2		1.364855

				366.22		1.364855

				366.24		1.364855

				366.26		1.364855

				366.28		1.364855

				366.31		1.364855

				366.33		1.364855

				366.35		1.364855

				366.37		1.364855

				366.39		1.364855

				366.41		1.364855

				366.43		1.364855

				366.45		1.364855

				366.48		1.364855

				366.5		1.364855

				366.52		1.364855

				366.54		1.364855

				366.56		1.364855

				366.58		1.364855

				366.6		1.364855

				366.62		1.364855

				366.65		1.364855

				366.67		1.364855

				366.69		1.364855

				366.71		1.364855

				366.73		1.364855

				366.75		1.364855

				366.77		1.364855

				366.79		1.364855

				366.82		1.364855

				366.84		1.364855

				366.86		1.364855

				366.88		1.364855

				366.9		1.364855

				366.92		1.364855

				366.94		1.364855

				366.96		1.364855

				366.99		1.364855

				367.01		1.364855

				367.03		1.364855

				367.05		1.364855

				367.07		1.364855

				367.09		1.364855

				367.11		1.364855

				367.13		1.364855

				367.15		1.364855

				367.18		1.364855

				367.2		1.364855

				367.22		1.364855

				367.24		1.364855

				367.26		1.368917

				367.28		1.368917

				367.3		1.368917

				367.32		1.368917

				367.35		1.368917

				367.37		1.368917

				367.39		1.368917

				367.41		1.368917

				367.43		1.368917

				367.45		1.368917

				367.47		1.368917

				367.49		1.368917

				367.52		1.364855

				367.54		1.368917

				367.56		1.364855

				367.58		1.364855

				367.6		1.364855

				367.62		1.364855

				367.64		1.364855

				367.66		1.364855

				367.68		1.364855

				367.71		1.364855

				367.73		1.364855

				367.75		1.364855

				367.77		1.364855

				367.79		1.364855

				367.81		1.364855

				367.83		1.364855

				367.85		1.364855

				367.88		1.364855

				367.9		1.364855

				367.92		1.364855

				367.94		1.364855

				367.96		1.364855

				367.98		1.364855

				368		1.364855

				368.02		1.364855

				368.05		1.364855

				368.07		1.364855

				368.09		1.364855

				368.11		1.364855

				368.13		1.364855

				368.15		1.364855

				368.17		1.364855

				368.19		1.364855

				368.22		1.364855

				368.24		1.364855

				368.26		1.364855

				368.28		1.364855

				368.3		1.364855

				368.32		1.364855

				368.34		1.364855

				368.36		1.364855

				368.39		1.364855

				368.41		1.364855

				368.43		1.364855

				368.45		1.364855

				368.47		1.364855

				368.49		1.364855

				368.51		1.364855

				368.53		1.364855

				368.55		1.364855

				368.58		1.364855

				368.6		1.364855

				368.62		1.364855

				368.64		1.364855

				368.66		1.364855

				368.68		1.364855

				368.7		1.364855

				368.72		1.364855

				368.75		1.364855

				368.77		1.364855

				368.79		1.364855

				368.81		1.364855

				368.83		1.364855

				368.85		1.364855

				368.87		1.364855

				368.89		1.364855

				368.92		1.364855

				368.94		1.364855

				368.96		1.364855

				368.98		1.364855

				369		1.364855

				369.02		1.364855

				369.04		1.364855

				369.06		1.364855

				369.09		1.360793

				369.11		1.360793

				369.13		1.360793

				369.15		1.360793

				369.17		1.360793

				369.19		1.360793

				369.21		1.360793

				369.23		1.360793

				369.26		1.360793

				369.28		1.360793

				369.3		1.360793

				369.32		1.360793

				369.34		1.360793

				369.36		1.360793

				369.38		1.360793

				369.4		1.360793

				369.42		1.360793

				369.45		1.360793

				369.47		1.360793

				369.49		1.360793

				369.51		1.360793

				369.53		1.360793

				369.55		1.360793

				369.57		1.360793

				369.59		1.360793

				369.62		1.360793

				369.64		1.360793

				369.66		1.360793

				369.68		1.360793

				369.7		1.360793

				369.72		1.360793

				369.74		1.360793

				369.76		1.360793

				369.79		1.360793

				369.81		1.360793

				369.83		1.360793

				369.85		1.360793

				369.87		1.360793

				369.89		1.360793

				369.91		1.360793

				369.93		1.360793

				369.96		1.360793

				369.98		1.360793

				370		1.360793

				370.02		1.360793

				370.04		1.360793

				370.06		1.360793

				370.08		1.360793

				370.1		1.360793

				370.13		1.360793

				370.15		1.360793

				370.17		1.360793

				370.19		1.360793

				370.21		1.360793

				370.23		1.360793

				370.25		1.360793

				370.28		1.360793

				370.3		1.360793

				370.32		1.360793

				370.34		1.360793

				370.36		1.360793

				370.38		1.360793

				370.4		1.360793

				370.42		1.360793

				370.45		1.360793

				370.47		1.360793

				370.49		1.360793

				370.51		1.360793

				370.53		1.360793

				370.55		1.360793

				370.57		1.360793

				370.59		1.360793

				370.62		1.360793

				370.64		1.360793

				370.66		1.360793

				370.68		1.360793

				370.7		1.360793

				370.72		1.360793

				370.74		1.360793

				370.76		1.360793

				370.78		1.360793

				370.81		1.360793

				370.83		1.360793

				370.85		1.360793

				370.87		1.360793

				370.89		1.360793

				370.91		1.360793

				370.93		1.360793

				370.95		1.360793

				370.98		1.360793

				371		1.360793

				371.02		1.360793

				371.04		1.360793

				371.06		1.360793

				371.08		1.360793

				371.1		1.360793

				371.12		1.360793

				371.15		1.360793

				371.17		1.360793

				371.19		1.360793

				371.21		1.360793

				371.23		1.360793

				371.25		1.360793

				371.27		1.360793

				371.29		1.360793

				371.32		1.364855

				371.34		1.364855

				371.36		1.364855

				371.38		1.364855

				371.4		1.364855

				371.42		1.364855

				371.44		1.364855

				371.46		1.364855

				371.49		1.364855

				371.51		1.364855

				371.53		1.364855

				371.55		1.364855

				371.57		1.364855

				371.59		1.364855

				371.61		1.364855

				371.63		1.364855

				371.66		1.364855

				371.68		1.364855

				371.7		1.364855

				371.72		1.364855

				371.74		1.364855

				371.76		1.364855

				371.78		1.364855

				371.8		1.364855

				371.83		1.364855

				371.85		1.364855

				371.87		1.364855

				371.89		1.364855

				371.91		1.364855

				371.93		1.364855

				371.95		1.364855

				371.97		1.364855

				372		1.364855

				372.02		1.364855

				372.04		1.364855

				372.06		1.364855

				372.08		1.364855

				372.1		1.364855

				372.12		1.364855

				372.15		1.364855

				372.17		1.364855

				372.19		1.364855

				372.21		1.364855

				372.23		1.364855

				372.25		1.364855

				372.27		1.364855

				372.29		1.364855

				372.32		1.364855

				372.34		1.364855

				372.36		1.364855

				372.38		1.364855

				372.4		1.364855

				372.42		1.364855

				372.44		1.364855

				372.46		1.364855

				372.49		1.364855

				372.51		1.364855

				372.53		1.364855

				372.55		1.364855

				372.57		1.364855

				372.59		1.364855

				372.61		1.364855

				372.63		1.364855

				372.66		1.364855

				372.68		1.364855

				372.7		1.364855

				372.72		1.364855

				372.74		1.364855

				372.76		1.364855

				372.78		1.364855

				372.8		1.364855

				372.83		1.364855

				372.85		1.364855

				372.87		1.364855

				372.89		1.364855

				372.91		1.364855

				372.93		1.364855

				372.95		1.364855

				372.97		1.364855

				373		1.364855

				373.02		1.364855

				373.04		1.364855

				373.06		1.364855

				373.08		1.364855

				373.1		1.364855

				373.12		1.364855

				373.14		1.364855

				373.17		1.364855

				373.19		1.364855

				373.21		1.364855

				373.23		1.364855

				373.25		1.364855

				373.27		1.364855

				373.29		1.364855

				373.31		1.364855

				373.34		1.364855

				373.36		1.364855

				373.38		1.364855

				373.4		1.364855

				373.42		1.364855

				373.44		1.364855

				373.46		1.364855

				373.48		1.364855

				373.51		1.364855

				373.53		1.364855

				373.55		1.364855

				373.57		1.364855

				373.59		1.364855

				373.61		1.364855

				373.63		1.364855

				373.65		1.364855

				373.68		1.364855

				373.7		1.364855

				373.72		1.364855

				373.74		1.364855

				373.76		1.364855

				373.78		1.364855

				373.8		1.364855

				373.82		1.364855

				373.85		1.364855

				373.87		1.364855

				373.89		1.364855

				373.91		1.364855

				373.93		1.364855

				373.95		1.364855

				373.97		1.360793

				373.99		1.360793

				374.02		1.360793

				374.04		1.360793

				374.06		1.360793

				374.08		1.360793

				374.1		1.360793

				374.12		1.360793

				374.14		1.360793

				374.16		1.360793

				374.19		1.360793

				374.21		1.360793

				374.23		1.360793

				374.25		1.360793

				374.27		1.360793

				374.29		1.360793

				374.31		1.360793

				374.33		1.360793

				374.36		1.360793

				374.38		1.360793

				374.4		1.360793

				374.42		1.360793

				374.44		1.360793

				374.46		1.360793

				374.48		1.360793

				374.5		1.360793

				374.53		1.360793

				374.55		1.360793

				374.57		1.360793

				374.59		1.360793

				374.61		1.360793

				374.63		1.360793

				374.65		1.360793

				374.67		1.360793

				374.7		1.356731

				374.72		1.356731

				374.74		1.356731

				374.76		1.356731

				374.78		1.360793

				374.8		1.356731

				374.82		1.356731

				374.84		1.360793

				374.87		1.356731

				374.89		1.360793

				374.91		1.356731

				374.93		1.356731

				374.95		1.356731

				374.97		1.356731

				374.99		1.356731

				375.01		1.356731

				375.04		1.356731

				375.06		1.356731

				375.08		1.356731

				375.1		1.356731

				375.12		1.356731

				375.14		1.356731

				375.16		1.356731

				375.18		1.356731

				375.21		1.356731

				375.23		1.356731

				375.25		1.356731

				375.27		1.356731

				375.29		1.356731

				375.31		1.356731

				375.33		1.356731

				375.35		1.356731

				375.38		1.356731

				375.4		1.356731

				375.42		1.360793

				375.44		1.360793

				375.46		1.360793

				375.48		1.360793

				375.5		1.360793

				375.52		1.360793

				375.55		1.360793

				375.57		1.360793

				375.59		1.360793

				375.61		1.360793

				375.63		1.360793

				375.65		1.360793

				375.67		1.360793

				375.69		1.360793

				375.72		1.360793

				375.74		1.360793

				375.76		1.360793

				375.78		1.360793

				375.8		1.360793

				375.82		1.360793

				375.84		1.360793

				375.86		1.360793

				375.89		1.360793

				375.91		1.360793

				375.93		1.360793

				375.95		1.360793

				375.97		1.360793

				375.99		1.360793

				376.01		1.360793

				376.03		1.360793

				376.06		1.360793

				376.08		1.360793

				376.1		1.360793

				376.12		1.364855

				376.14		1.360793

				376.16		1.360793

				376.18		1.360793

				376.2		1.360793

				376.23		1.360793

				376.25		1.360793

				376.27		1.360793

				376.29		1.360793

				376.31		1.360793

				376.33		1.360793

				376.35		1.360793

				376.37		1.360793

				376.4		1.360793

				376.42		1.360793

				376.44		1.364855

				376.46		1.364855

				376.48		1.368917

				376.5		1.364855

				376.52		1.364855

				376.54		1.364855

				376.57		1.364855

				376.59		1.364855

				376.61		1.364855

				376.63		1.364855

				376.65		1.364855

				376.67		1.364855

				376.69		1.364855

				376.72		1.364855

				376.74		1.364855

				376.76		1.364855

				376.78		1.364855

				376.8		1.364855

				376.82		1.364855

				376.84		1.364855

				376.86		1.364855

				376.89		1.364855

				376.91		1.364855

				376.93		1.364855

				376.95		1.360793

				376.97		1.360793

				376.99		1.360793

				377.01		1.364855

				377.03		1.364855

				377.06		1.364855

				377.08		1.364855

				377.1		1.364855

				377.12		1.364855

				377.14		1.364855

				377.16		1.364855

				377.18		1.364855

				377.2		1.364855

				377.23		1.364855

				377.25		1.364855

				377.27		1.364855

				377.29		1.364855

				377.31		1.364855

				377.33		1.364855

				377.35		1.364855

				377.37		1.364855

				377.4		1.364855

				377.42		1.364855

				377.44		1.364855

				377.46		1.364855

				377.48		1.364855

				377.5		1.364855

				377.52		1.364855

				377.54		1.364855

				377.57		1.364855

				377.59		1.364855

				377.61		1.364855

				377.63		1.364855

				377.65		1.364855

				377.67		1.364855

				377.69		1.364855

				377.71		1.364855

				377.74		1.364855

				377.76		1.364855

				377.78		1.364855

				377.8		1.364855

				377.82		1.364855

				377.84		1.364855

				377.86		1.364855

				377.88		1.364855

				377.91		1.364855

				377.93		1.364855

				377.95		1.364855

				377.97		1.364855

				377.99		1.364855

				378.01		1.364855

				378.03		1.364855

				378.05		1.364855

				378.07		1.364855

				378.1		1.364855

				378.12		1.364855

				378.14		1.364855

				378.16		1.364855

				378.18		1.368917

				378.2		1.368917

				378.22		1.364855

				378.24		1.368917

				378.27		1.368917

				378.29		1.368917

				378.31		1.368917

				378.33		1.368917

				378.35		1.368917

				378.37		1.368917

				378.39		1.368917

				378.41		1.368917

				378.44		1.368917

				378.46		1.368917

				378.48		1.368917

				378.5		1.368917

				378.52		1.368917

				378.54		1.368917

				378.56		1.368917

				378.58		1.364855

				378.61		1.364855

				378.63		1.364855

				378.65		1.368917

				378.67		1.368917

				378.69		1.368917

				378.71		1.368917

				378.73		1.368917

				378.75		1.368917

				378.77		1.368917

				378.8		1.368917

				378.82		1.368917

				378.84		1.368917

				378.86		1.368917

				378.88		1.368917

				378.9		1.368917

				378.92		1.368917

				378.94		1.368917

				378.97		1.368917

				378.99		1.372979

				379.01		1.368917

				379.03		1.372979

				379.05		1.372979

				379.07		1.372979

				379.09		1.372979

				379.11		1.368917

				379.14		1.368917

				379.16		1.368917

				379.18		1.368917

				379.2		1.368917

				379.22		1.368917

				379.24		1.368917

				379.26		1.372979

				379.28		1.368917

				379.3		1.368917

				379.33		1.372979

				379.35		1.372979

				379.37		1.372979

				379.39		1.372979

				379.41		1.372979

				379.43		1.372979

				379.45		1.368917

				379.47		1.372979

				379.5		1.372979

				379.52		1.372979

				379.54		1.372979

				379.56		1.372979

				379.58		1.372979

				379.6		1.372979

				379.62		1.372979

				379.64		1.372979

				379.67		1.372979

				379.69		1.368917

				379.71		1.368917

				379.73		1.368917

				379.75		1.372979

				379.77		1.372979

				379.79		1.372979

				379.81		1.372979

				379.84		1.372979

				379.86		1.372979

				379.88		1.372979

				379.9		1.372979

				379.92		1.372979

				379.94		1.372979

				379.96		1.372979

				379.98		1.372979

				380.01		1.372979

				380.03		1.372979

				380.05		1.372979

				380.07		1.372979

				380.09		1.368917

				380.11		1.372979

				380.13		1.368917

				380.15		1.372979

				380.18		1.372979

				380.2		1.372979

				380.22		1.372979

				380.24		1.372979

				380.26		1.372979

				380.28		1.372979

				380.3		1.372979

				380.32		1.372979

				380.35		1.372979

				380.37		1.372979

				380.39		1.372979

				380.41		1.372979

				380.43		1.372979

				380.45		1.372979

				380.47		1.372979

				380.49		1.372979

				380.52		1.372979

				380.54		1.372979

				380.56		1.372979

				380.58		1.372979

				380.6		1.372979

				380.62		1.372979

				380.64		1.372979

				380.66		1.372979

				380.68		1.372979

				380.71		1.372979

				380.73		1.372979

				380.75		1.372979

				380.77		1.372979

				380.79		1.372979

				380.81		1.372979

				380.83		1.372979

				380.85		1.372979

				380.88		1.372979

				380.9		1.372979

				380.92		1.377041

				380.94		1.372979

				380.96		1.377041

				380.98		1.377041

				381		1.377041

				381.02		1.377041

				381.05		1.377041

				381.07		1.377041

				381.09		1.377041

				381.11		1.377041

				381.13		1.377041

				381.15		1.377041

				381.17		1.377041

				381.19		1.377041

				381.22		1.377041

				381.24		1.377041

				381.26		1.377041

				381.28		1.377041

				381.3		1.377041

				381.32		1.377041

				381.34		1.377041

				381.36		1.377041

				381.39		1.377041

				381.41		1.377041

				381.43		1.377041

				381.45		1.377041

				381.47		1.377041

				381.49		1.377041

				381.51		1.377041

				381.53		1.377041

				381.55		1.377041

				381.58		1.377041

				381.6		1.377041

				381.62		1.377041

				381.64		1.377041

				381.66		1.377041

				381.68		1.377041

				381.7		1.377041

				381.72		1.377041

				381.75		1.377041

				381.77		1.377041

				381.79		1.377041

				381.81		1.377041

				381.83		1.377041

				381.85		1.377041

				381.87		1.377041

				381.89		1.377041

				381.92		1.377041

				381.94		1.377041

				381.96		1.377041

				381.98		1.377041

				382		1.377041

				382.02		1.377041

				382.04		1.377041

				382.06		1.377041

				382.09		1.377041

				382.11		1.377041

				382.13		1.377041

				382.15		1.377041

				382.17		1.377041

				382.19		1.377041

				382.21		1.377041

				382.23		1.377041

				382.25		1.377041

				382.28		1.377041

				382.3		1.377041

				382.32		1.377041

				382.34		1.377041

				382.36		1.377041

				382.38		1.377041

				382.4		1.372979

				382.42		1.372979

				382.45		1.372979

				382.47		1.372979

				382.49		1.372979

				382.51		1.372979

				382.53		1.372979

				382.55		1.372979

				382.57		1.372979

				382.59		1.372979

				382.62		1.372979

				382.64		1.372979

				382.66		1.372979

				382.68		1.372979

				382.7		1.372979

				382.72		1.372979

				382.74		1.372979

				382.76		1.372979

				382.78		1.368917

				382.81		1.368917

				382.83		1.368917

				382.85		1.368917

				382.87		1.368917

				382.89		1.368917

				382.91		1.368917

				382.93		1.368917

				382.95		1.368917

				382.98		1.368917

				383		1.368917

				383.02		1.368917

				383.04		1.368917

				383.06		1.368917

				383.08		1.368917

				383.1		1.368917

				383.12		1.368917

				383.15		1.364855

				383.17		1.364855

				383.19		1.364855

				383.21		1.364855

				383.23		1.364855

				383.25		1.364855

				383.27		1.364855

				383.29		1.364855

				383.32		1.364855

				383.34		1.364855

				383.36		1.364855

				383.38		1.360793

				383.4		1.360793

				383.42		1.360793

				383.44		1.360793

				383.46		1.360793

				383.48		1.360793

				383.51		1.360793

				383.53		1.360793

				383.55		1.360793

				383.57		1.360793

				383.59		1.360793

				383.61		1.360793

				383.63		1.360793

				383.65		1.360793

				383.68		1.356731

				383.7		1.360793

				383.72		1.360793

				383.74		1.356731

				383.76		1.360793

				383.78		1.360793

				383.8		1.360793

				383.82		1.360793

				383.85		1.360793

				383.87		1.360793

				383.89		1.360793

				383.91		1.360793

				383.93		1.360793

				383.95		1.360793

				383.97		1.360793

				383.99		1.360793

				384.02		1.360793

				384.04		1.360793

				384.06		1.360793

				384.08		1.360793

				384.1		1.360793

				384.12		1.360793

				384.14		1.360793

				384.16		1.360793

				384.19		1.360793

				384.21		1.360793

				384.23		1.360793

				384.25		1.360793

				384.27		1.360793

				384.29		1.360793

				384.31		1.360793

				384.33		1.360793

				384.35		1.360793

				384.38		1.364855

				384.4		1.364855

				384.42		1.364855

				384.44		1.360793

				384.46		1.360793

				384.48		1.360793

				384.5		1.360793

				384.52		1.360793

				384.55		1.360793

				384.57		1.360793

				384.59		1.360793

				384.61		1.360793

				384.63		1.360793

				384.65		1.360793

				384.67		1.360793

				384.69		1.360793

				384.71		1.360793

				384.74		1.360793

				384.76		1.360793

				384.78		1.360793

				384.8		1.360793

				384.82		1.364855

				384.84		1.364855

				384.86		1.364855

				384.88		1.364855

				384.91		1.364855

				384.93		1.364855

				384.95		1.364855

				384.97		1.364855

				384.99		1.360793

				385.01		1.364855

				385.03		1.368917

				385.05		1.364855

				385.07		1.364855

				385.1		1.364855

				385.12		1.364855

				385.14		1.364855

				385.16		1.368917

				385.18		1.368917

				385.2		1.368917

				385.22		1.368917

				385.24		1.368917

				385.27		1.368917

				385.29		1.368917

				385.31		1.368917

				385.33		1.368917

				385.35		1.368917

				385.37		1.368917

				385.39		1.372979

				385.41		1.372979

				385.43		1.372979

				385.46		1.372979

				385.48		1.372979

				385.5		1.372979

				385.52		1.372979

				385.54		1.372979

				385.56		1.372979

				385.58		1.372979

				385.6		1.372979

				385.62		1.372979

				385.65		1.372979

				385.67		1.372979

				385.69		1.377041

				385.71		1.377041

				385.73		1.377041

				385.75		1.377041

				385.77		1.377041

				385.79		1.377041

				385.82		1.377041

				385.84		1.377041

				385.86		1.377041

				385.88		1.377041

				385.9		1.377041

				385.92		1.381103

				385.94		1.377041

				385.96		1.377041

				385.98		1.377041

				386.01		1.377041

				386.03		1.377041

				386.05		1.377041

				386.07		1.377041

				386.09		1.377041

				386.11		1.377041

				386.13		1.377041

				386.15		1.377041

				386.18		1.377041

				386.2		1.377041

				386.22		1.377041

				386.24		1.377041

				386.26		1.377041

				386.28		1.377041

				386.3		1.377041

				386.32		1.377041

				386.34		1.377041

				386.37		1.377041

				386.39		1.377041

				386.41		1.381103

				386.43		1.381103

				386.45		1.377041

				386.47		1.377041

				386.49		1.377041

				386.51		1.377041

				386.54		1.381103

				386.56		1.381103

				386.58		1.381103

				386.6		1.381103

				386.62		1.381103

				386.64		1.381103

				386.66		1.381103

				386.68		1.381103

				386.71		1.381103

				386.73		1.381103

				386.75		1.381103

				386.77		1.381103

				386.79		1.381103

				386.81		1.385165

				386.83		1.385165

				386.85		1.381103

				386.87		1.385165

				386.9		1.385165

				386.92		1.385165

				386.94		1.385165

				386.96		1.381103

				386.98		1.385165

				387		1.385165

				387.02		1.385165

				387.04		1.385165

				387.07		1.385165

				387.09		1.385165

				387.11		1.385165

				387.13		1.381103

				387.15		1.385165

				387.17		1.385165

				387.19		1.381103

				387.21		1.381103

				387.23		1.381103

				387.26		1.381103

				387.28		1.381103

				387.3		1.381103

				387.32		1.381103

				387.34		1.381103

				387.36		1.381103

				387.38		1.381103

				387.4		1.381103

				387.43		1.381103

				387.45		1.381103

				387.47		1.381103

				387.49		1.381103

				387.51		1.381103

				387.53		1.381103

				387.55		1.381103

				387.57		1.381103

				387.6		1.381103

				387.62		1.381103

				387.64		1.381103

				387.66		1.381103

				387.68		1.381103

				387.7		1.381103

				387.72		1.381103

				387.74		1.381103

				387.76		1.381103

				387.79		1.381103

				387.81		1.381103

				387.83		1.381103

				387.85		1.381103

				387.87		1.381103

				387.89		1.381103

				387.91		1.381103

				387.93		1.381103

				387.96		1.381103

				387.98		1.381103

				388		1.381103

				388.02		1.381103

				388.04		1.381103

				388.06		1.381103

				388.08		1.381103

				388.1		1.381103

				388.12		1.381103

				388.15		1.381103

				388.17		1.381103

				388.19		1.381103

				388.21		1.385165

				388.23		1.385165

				388.25		1.381103

				388.27		1.385165

				388.29		1.385165

				388.31		1.385165

				388.34		1.385165

				388.36		1.385165

				388.38		1.385165

				388.4		1.381103

				388.42		1.385165

				388.44		1.385165

				388.46		1.381103

				388.48		1.385165

				388.51		1.385165

				388.53		1.385165

				388.55		1.385165

				388.57		1.381103

				388.59		1.381103

				388.61		1.381103

				388.63		1.381103

				388.65		1.381103

				388.67		1.381103

				388.7		1.381103

				388.72		1.381103

				388.74		1.381103

				388.76		1.381103

				388.78		1.381103

				388.8		1.381103

				388.82		1.381103

				388.84		1.381103

				388.87		1.381103

				388.89		1.381103

				388.91		1.381103

				388.93		1.381103

				388.95		1.381103

				388.97		1.381103

				388.99		1.381103

				389.01		1.381103

				389.03		1.381103

				389.06		1.381103

				389.08		1.381103

				389.1		1.381103

				389.12		1.381103

				389.14		1.381103

				389.16		1.381103

				389.18		1.381103

				389.2		1.381103

				389.23		1.381103

				389.25		1.381103

				389.27		1.381103

				389.29		1.381103

				389.31		1.381103

				389.33		1.381103

				389.35		1.381103

				389.37		1.381103

				389.39		1.381103

				389.42		1.381103

				389.44		1.381103

				389.46		1.381103

				389.48		1.381103

				389.5		1.381103

				389.52		1.381103

				389.54		1.381103

				389.56		1.381103

				389.59		1.381103

				389.61		1.381103

				389.63		1.381103

				389.65		1.381103

				389.67		1.381103

				389.69		1.381103

				389.71		1.381103

				389.73		1.381103

				389.75		1.381103

				389.78		1.381103

				389.8		1.381103

				389.82		1.381103

				389.84		1.381103

				389.86		1.381103

				389.88		1.381103

				389.9		1.381103

				389.92		1.381103

				389.95		1.381103

				389.97		1.381103

				389.99		1.381103

				390.01		1.381103

				390.03		1.381103

				390.05		1.381103

				390.07		1.381103

				390.09		1.377041

				390.11		1.377041

				390.14		1.377041

				390.16		1.377041

				390.18		1.377041

				390.2		1.377041

				390.22		1.377041

				390.24		1.377041

				390.26		1.377041

				390.28		1.377041

				390.31		1.377041

				390.33		1.377041

				390.35		1.377041

				390.37		1.377041

				390.39		1.377041

				390.41		1.377041

				390.43		1.377041

				390.45		1.377041

				390.48		1.377041

				390.5		1.377041

				390.52		1.377041

				390.54		1.377041

				390.56		1.377041

				390.58		1.377041

				390.6		1.377041

				390.62		1.377041

				390.64		1.377041

				390.67		1.377041

				390.69		1.377041

				390.71		1.377041

				390.73		1.377041

				390.75		1.377041

				390.77		1.377041

				390.79		1.377041

				390.81		1.377041

				390.84		1.377041

				390.86		1.377041

				390.88		1.377041

				390.9		1.377041

				390.92		1.377041

				390.94		1.377041

				390.96		1.377041

				390.98		1.377041

				391		1.377041

				391.03		1.377041

				391.05		1.377041

				391.07		1.377041

				391.09		1.377041

				391.11		1.377041

				391.13		1.377041

				391.15		1.377041

				391.17		1.377041

				391.2		1.377041

				391.22		1.377041

				391.24		1.377041

				391.26		1.377041

				391.28		1.377041

				391.3		1.377041

				391.32		1.377041

				391.34		1.377041

				391.36		1.377041

				391.39		1.377041

				391.41		1.377041

				391.43		1.377041

				391.45		1.377041

				391.47		1.377041

				391.49		1.377041

				391.51		1.377041

				391.53		1.377041

				391.56		1.377041

				391.58		1.377041

				391.6		1.377041

				391.62		1.377041

				391.64		1.377041

				391.66		1.377041

				391.68		1.377041

				391.7		1.377041

				391.72		1.381103

				391.75		1.377041

		Results:

		Onset		X1		188.9		°C

				Y1		95.776		%

				X2		255.23		°C

				Y2		14.38		%

				Onset X		219.95		°C

				Onset Y		83.163		%
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		Method Filename:		C:\Program Files (x86)\PerkinElmer\Pyris\data\Anas\21052024\RT54-MWCNT 0.2 (GNP 0.75-MW 0.25).t6d

		Sample ID:		RT54-MWCNT 0.2 (GNP 0.75-MW 0.25)

		Step:		1

		Data		Sample Temperature (°C)		Weight % (%)

				30.07		100

				30.07		100

				30.07		100

				30.07		100

				30.07		100

				30.07		100.006

				30.07		100.006

				30.07		100

				30.07		100.006

				30.07		100.006

				30.07		100.006

				30.07		100.006

				30.07		100.006

				30.07		100

				30.07		100.006

				30.07		100.006

				30.07		100.006

				30.07		100.006

				30.07		100.006

				30.07		100.006

				30.07		100.006

				30.07		100.006

				30.07		100.006

				30.07		100.006

				30.07		100.006

				30.06		100.006

				30.06		100.006

				30.06		100.006

				30.06		100.006

				30.06		100.006

				30.06		100.006

				30.06		100.006

				30.06		100.006

				30.06		100.006

				30.06		100.006

				30.06		100.006

				30.06		100.006

				30.06		100.006

				30.06		100.006

				30.06		100.006

				30.06		100.006

				30.06		100.0119

				30.06		100.0119

				30.06		100.0119

				30.06		100.0119

				30.06		100.0119

				30.06		100.0119

				30.06		100.0119

				30.06		100.0119

				30.06		100.0119

				30.06		100.0119

				30.06		100.0119

				30.06		100.0119

				30.06		100.0119

				30.06		100.0119

				30.06		100.0179

				30.06		100.0179

				30.06		100.0179

				30.06		100.0179

				30.06		100.0179

				30.06		100.0179

				30.06		100.0179

				30.06		100.0179

				30.06		100.0239

				30.06		100.0179

				30.06		100.0179

				30.06		100.0179

				30.06		100.0119

				30.06		100.0119

				30.06		100.0119

				30.06		100.0179

				30.06		100.0119

				30.06		100.0119

				30.06		100.0179

				30.06		100.0179

				30.06		100.0179

				30.06		100.0179

				30.06		100.0179

				30.06		100.0179

				30.06		100.0179

				30.06		100.0179

				30.06		100.0179

				30.06		100.0179

				30.06		100.0179

				30.06		100.0179

				30.06		100.0179

				30.06		100.0179

				30.06		100.0179

				30.06		100.0179

				30.06		100.0239

				30.06		100.0239

				30.06		100.0239

				30.06		100.0239

				30.06		100.0239

				30.06		100.0239

				30.06		100.0299

				30.06		100.0299

				30.06		100.0299

				30.06		100.0299

				30.06		100.0299

				30.06		100.0299

				30.06		100.0299

				30.06		100.0299

				30.06		100.0358

				30.06		100.0358

				30.06		100.0358

				30.07		100.0358

				30.07		100.0358

				30.07		100.0358

				30.07		100.0358

				30.07		100.0358

				30.07		100.0358

				30.07		100.0418

				30.07		100.0418

				30.07		100.0418

				30.07		100.0418

				30.07		100.0418

				30.07		100.0418

				30.07		100.0418

				30.07		100.0418

				30.07		100.0478

				30.08		100.0478

				30.08		100.0478

				30.08		100.0478

				30.08		100.0478

				30.08		100.0478

				30.08		100.0538

				30.08		100.0478

				30.08		100.0538

				30.08		100.0538

				30.08		100.0538

				30.09		100.0538

				30.09		100.0538

				30.09		100.0597

				30.09		100.0597

				30.09		100.0597

				30.09		100.0597

				30.09		100.0597

				30.1		100.0597

				30.1		100.0597

				30.1		100.0597

				30.1		100.0657

				30.1		100.0657

				30.1		100.0657

				30.11		100.0657

				30.11		100.0657

				30.11		100.0657

				30.11		100.0657

				30.11		100.0657

				30.11		100.0657

				30.12		100.0657

				30.12		100.0657

				30.12		100.0657

				30.12		100.0657

				30.13		100.0657

				30.13		100.0657

				30.13		100.0717

				30.13		100.0717

				30.13		100.0717

				30.14		100.0717

				30.14		100.0717

				30.14		100.0717

				30.14		100.0717

				30.15		100.0777

				30.15		100.0777

				30.15		100.0777

				30.15		100.0836

				30.16		100.0836

				30.16		100.0836

				30.16		100.0836

				30.17		100.0836

				30.17		100.0896

				30.17		100.0836

				30.17		100.0896

				30.18		100.0896

				30.18		100.0896

				30.18		100.0896

				30.19		100.0896

				30.19		100.0896

				30.19		100.0896

				30.2		100.0896

				30.2		100.0896

				30.2		100.0956

				30.21		100.0956

				30.21		100.0956

				30.21		100.0956

				30.22		100.0956

				30.22		100.0956

				30.23		100.0956

				30.23		100.0956

				30.23		100.0956

				30.24		100.0956

				30.24		100.0956

				30.24		100.0956

				30.25		100.0956

				30.25		100.0956

				30.26		100.0956

				30.26		100.0956

				30.26		100.0956

				30.27		100.0956

				30.27		100.0956

				30.28		100.0956

				30.28		100.0956

				30.29		100.0956

				30.29		100.0956

				30.29		100.0956

				30.3		100.1016

				30.3		100.1016

				30.31		100.1016

				30.31		100.1016

				30.32		100.1016

				30.32		100.1016

				30.33		100.1016

				30.33		100.1016

				30.33		100.1016

				30.34		100.1016

				30.34		100.1016

				30.35		100.1016

				30.35		100.1016

				30.36		100.1016

				30.36		100.1016

				30.37		100.1016

				30.37		100.1075

				30.38		100.1075

				30.38		100.1075

				30.39		100.1075

				30.39		100.1075

				30.4		100.1075

				30.4		100.1075

				30.41		100.1075

				30.42		100.1075

				30.42		100.1075

				30.43		100.1075

				30.43		100.1075

				30.44		100.1075

				30.44		100.1075

				30.45		100.1075

				30.45		100.1135

				30.46		100.1135

				30.46		100.1135

				30.47		100.1135

				30.48		100.1135

				30.48		100.1135

				30.49		100.1135

				30.49		100.1135

				30.5		100.1135

				30.51		100.1135

				30.51		100.1195

				30.52		100.1195

				30.52		100.1195

				30.53		100.1195

				30.54		100.1195

				30.54		100.1195

				30.55		100.1195

				30.55		100.1195

				30.56		100.1195

				30.57		100.1195

				30.57		100.1195

				30.58		100.1195

				30.58		100.1195

				30.59		100.1195

				30.6		100.1195

				30.6		100.1254

				30.61		100.1254

				30.62		100.1254

				30.62		100.1254

				30.63		100.1254

				30.64		100.1254

				30.64		100.1254

				30.65		100.1254

				30.66		100.1254

				30.66		100.1254

				30.67		100.1254

				30.68		100.1254

				30.68		100.1254

				30.69		100.1254

				30.7		100.1314

				30.7		100.1314

				30.71		100.1314

				30.72		100.1314

				30.72		100.1314

				30.73		100.1314

				30.74		100.1314

				30.75		100.1314

				30.75		100.1314

				30.76		100.1314

				30.77		100.1374

				30.77		100.1374

				30.78		100.1374

				30.79		100.1374

				30.8		100.1374

				30.8		100.1374

				30.81		100.1374

				30.82		100.1374

				30.83		100.1374

				30.83		100.1434

				30.84		100.1374

				30.85		100.1374

				30.85		100.1434

				30.86		100.1434

				30.87		100.1434

				30.88		100.1374

				30.88		100.1434

				30.89		100.1434

				30.9		100.1434

				30.91		100.1434

				30.92		100.1434

				30.92		100.1434

				30.93		100.1434

				30.94		100.1434

				30.95		100.1434

				30.95		100.1434

				30.96		100.1434

				30.97		100.1434

				30.98		100.1434

				30.99		100.1493

				30.99		100.1493

				31		100.1493

				31.01		100.1493

				31.02		100.1493

				31.03		100.1493

				31.03		100.1493

				31.04		100.1493

				31.05		100.1493

				31.06		100.1493

				31.07		100.1493

				31.07		100.1493

				31.08		100.1493

				31.09		100.1493

				31.1		100.1493

				31.11		100.1493

				31.12		100.1493

				31.12		100.1493

				31.13		100.1493

				31.14		100.1493

				31.15		100.1493

				31.16		100.1493

				31.17		100.1493

				31.17		100.1493

				31.18		100.1493

				31.19		100.1553

				31.2		100.1553

				31.21		100.1553

				31.22		100.1553

				31.23		100.1553

				31.23		100.1553

				31.24		100.1553

				31.25		100.1553

				31.26		100.1553

				31.27		100.1553

				31.28		100.1553

				31.29		100.1553

				31.3		100.1553

				31.3		100.1553

				31.31		100.1553

				31.32		100.1553

				31.33		100.1553

				31.34		100.1553

				31.35		100.1553

				31.36		100.1553

				31.37		100.1553

				31.38		100.1553

				31.38		100.1553

				31.39		100.1553

				31.4		100.1553

				31.41		100.1553

				31.42		100.1553

				31.43		100.1613

				31.44		100.1613

				31.45		100.1613

				31.46		100.1613

				31.47		100.1613

				31.48		100.1613

				31.49		100.1613

				31.49		100.1613

				31.5		100.1613

				31.51		100.1613

				31.52		100.1613

				31.53		100.1613

				31.54		100.1613

				31.55		100.1613

				31.56		100.1613

				31.57		100.1613

				31.58		100.1613

				31.59		100.1613

				31.6		100.1613

				31.61		100.1613

				31.62		100.1613

				31.63		100.1613

				31.64		100.1613

				31.65		100.1613

				31.66		100.1613

				31.67		100.1613

				31.68		100.1613

				31.68		100.1613

				31.69		100.1613

				31.7		100.1613

				31.71		100.1613

				31.72		100.1613

				31.73		100.1613

				31.74		100.1613

				31.75		100.1613

				31.76		100.1613

				31.77		100.1673

				31.78		100.1673

				31.79		100.1673

				31.8		100.1673

				31.81		100.1673

				31.82		100.1673

				31.83		100.1673

				31.84		100.1673

				31.85		100.1673

				31.86		100.1673

				31.87		100.1673

				31.88		100.1673

				31.89		100.1673

				31.9		100.1673

				31.91		100.1673

				31.92		100.1673

				31.93		100.1673

				31.94		100.1673

				31.96		100.1673

				31.97		100.1673

				31.98		100.1673

				31.99		100.1673

				32		100.1673

				32.01		100.1732

				32.02		100.1732

				32.03		100.1732

				32.04		100.1732

				32.05		100.1732

				32.06		100.1732

				32.07		100.1732

				32.08		100.1732

				32.09		100.1732

				32.1		100.1732

				32.11		100.1732

				32.12		100.1732

				32.13		100.1732

				32.14		100.1732

				32.15		100.1732

				32.17		100.1732

				32.18		100.1732

				32.19		100.1792

				32.2		100.1792

				32.21		100.1792

				32.22		100.1792

				32.23		100.1792

				32.24		100.1792

				32.25		100.1792

				32.26		100.1792

				32.27		100.1792

				32.28		100.1792

				32.29		100.1792

				32.31		100.1792

				32.32		100.1792

				32.33		100.1792

				32.34		100.1792

				32.35		100.1792

				32.36		100.1792

				32.37		100.1792

				32.38		100.1792

				32.39		100.1792

				32.41		100.1792

				32.42		100.1792

				32.43		100.1792

				32.44		100.1852

				32.45		100.1792

				32.46		100.1852

				32.47		100.1852

				32.48		100.1852

				32.49		100.1852

				32.51		100.1852

				32.52		100.1852

				32.53		100.1852

				32.54		100.1852

				32.55		100.1852

				32.56		100.1852

				32.57		100.1852

				32.59		100.1852

				32.6		100.1852

				32.61		100.1852

				32.62		100.1852

				32.63		100.1852

				32.64		100.1852

				32.65		100.1852

				32.67		100.1852

				32.68		100.1852

				32.69		100.1852

				32.7		100.1852

				32.71		100.1852

				32.72		100.1912

				32.74		100.1912

				32.75		100.1852

				32.76		100.1912

				32.77		100.1912

				32.78		100.1912

				32.79		100.1912

				32.81		100.1912

				32.82		100.1912

				32.83		100.1852

				32.84		100.1912

				32.85		100.1912

				32.87		100.1912

				32.88		100.1912

				32.89		100.1912

				32.9		100.1912

				32.91		100.1912

				32.92		100.1912

				32.94		100.1912

				32.95		100.1912

				32.96		100.1912

				32.97		100.1912

				32.98		100.1912

				33		100.1912

				33.01		100.1912

				33.02		100.1912

				33.03		100.1912

				33.05		100.1912

				33.06		100.1912

				33.07		100.1912

				33.08		100.1912

				33.09		100.1912

				33.11		100.1912

				33.12		100.1912

				33.13		100.1912

				33.14		100.1971

				33.16		100.1971

				33.17		100.1971

				33.18		100.1971

				33.19		100.1971

				33.2		100.1971

				33.22		100.1971

				33.23		100.1971

				33.24		100.1971

				33.25		100.1971

				33.27		100.1971

				33.28		100.1971

				33.29		100.1971

				33.3		100.1971

				33.32		100.1971

				33.33		100.1971

				33.34		100.1971

				33.35		100.1971

				33.37		100.1971

				33.38		100.1971

				33.39		100.1971

				33.4		100.1971

				33.42		100.1971

				33.43		100.1971

				33.44		100.1971

				33.46		100.1971

				33.47		100.1971

				33.48		100.1971

				33.49		100.1971

				33.51		100.2031

				33.52		100.2031

				33.53		100.2031

				33.54		100.2031

				33.56		100.2031

				33.57		100.2031

				33.58		100.2031

				33.6		100.2031

				33.61		100.2031

				33.62		100.2031

				33.63		100.2031

				33.65		100.2031

				33.66		100.2031

				33.67		100.2031

				33.69		100.2031

				33.7		100.2031

				33.71		100.2031

				33.73		100.2031

				33.74		100.2031

				33.75		100.2031

				33.76		100.2031

				33.78		100.2031

				33.79		100.2031

				33.8		100.2031

				33.82		100.2031

				33.83		100.2031

				33.84		100.2031

				33.86		100.2031

				33.87		100.2091

				33.88		100.2091

				33.9		100.2091

				33.91		100.2091

				33.92		100.2091

				33.94		100.2091

				33.95		100.2091

				33.96		100.2091

				33.98		100.2091

				33.99		100.2091

				34		100.2091

				34.02		100.2091

				34.03		100.2091

				34.04		100.2091

				34.06		100.2151

				34.07		100.2151

				34.08		100.2151

				34.1		100.2151

				34.11		100.2151

				34.12		100.2151

				34.14		100.2151

				34.15		100.2151

				34.16		100.2151

				34.18		100.2151

				34.19		100.221

				34.2		100.2151

				34.22		100.221

				34.23		100.221

				34.25		100.221

				34.26		100.221

				34.27		100.221

				34.29		100.221

				34.3		100.221

				34.31		100.221

				34.33		100.221

				34.34		100.221

				34.35		100.221

				34.37		100.221

				34.38		100.221

				34.4		100.227

				34.41		100.227

				34.42		100.227

				34.44		100.227

				34.45		100.227

				34.47		100.227

				34.48		100.227

				34.49		100.227

				34.51		100.227

				34.52		100.227

				34.53		100.227

				34.55		100.227

				34.56		100.227

				34.58		100.233

				34.59		100.227

				34.6		100.233

				34.62		100.233

				34.63		100.233

				34.65		100.233

				34.66		100.233

				34.67		100.233

				34.69		100.233

				34.7		100.233

				34.72		100.233

				34.73		100.233

				34.74		100.233

				34.76		100.233

				34.77		100.2389

				34.79		100.233

				34.8		100.2389

				34.82		100.233

				34.83		100.233

				34.84		100.233

				34.86		100.2389

				34.87		100.2389

				34.89		100.2389

				34.9		100.2389

				34.92		100.2389

				34.93		100.2389

				34.94		100.2389

				34.96		100.2389

				34.97		100.2389

				34.99		100.2389

				35		100.2389

				35.02		100.2389

				35.03		100.2449

				35.04		100.2449

				35.06		100.2449

				35.07		100.2449

				35.09		100.2449

				35.1		100.2449

				35.12		100.2449

				35.13		100.2449

				35.15		100.2449

				35.16		100.2449

				35.17		100.2449

				35.19		100.2509

				35.2		100.2509

				35.22		100.2509

				35.23		100.2509

				35.25		100.2509

				35.26		100.2509

				35.28		100.2509

				35.29		100.2509

				35.31		100.2509

				35.32		100.2509

				35.34		100.2509

				35.35		100.2509

				35.36		100.2509

				35.38		100.2509

				35.39		100.2509

				35.41		100.2509

				35.42		100.2509

				35.44		100.2509

				35.45		100.2509

				35.47		100.2509

				35.48		100.2509

				35.5		100.2509

				35.51		100.2509

				35.53		100.2509

				35.54		100.2509

				35.56		100.2509

				35.57		100.2509

				35.59		100.2569

				35.6		100.2569

				35.62		100.2569

				35.63		100.2569

				35.65		100.2569

				35.66		100.2569

				35.68		100.2569

				35.69		100.2569

				35.71		100.2569

				35.72		100.2569

				35.74		100.2569

				35.75		100.2569

				35.77		100.2569

				35.78		100.2569

				35.8		100.2569

				35.81		100.2569

				35.83		100.2569

				35.84		100.2569

				35.86		100.2569

				35.87		100.2569

				35.89		100.2628

				35.9		100.2628

				35.92		100.2628

				35.93		100.2628

				35.95		100.2628

				35.96		100.2628

				35.98		100.2628

				35.99		100.2628

				36.01		100.2628

				36.02		100.2628

				36.04		100.2628

				36.05		100.2628

				36.07		100.2628

				36.08		100.2628

				36.1		100.2628

				36.11		100.2628

				36.13		100.2628

				36.14		100.2628

				36.16		100.2628

				36.18		100.2628

				36.19		100.2628

				36.21		100.2628

				36.22		100.2628

				36.24		100.2688

				36.25		100.2688

				36.27		100.2688

				36.28		100.2688

				36.3		100.2688

				36.31		100.2688

				36.33		100.2688

				36.34		100.2688

				36.36		100.2688

				36.38		100.2688

				36.39		100.2688

				36.41		100.2688

				36.42		100.2688

				36.44		100.2688

				36.45		100.2688

				36.47		100.2688

				36.48		100.2688

				36.5		100.2688

				36.52		100.2688

				36.53		100.2688

				36.55		100.2688

				36.56		100.2688

				36.58		100.2688

				36.59		100.2688

				36.61		100.2688

				36.62		100.2688

				36.64		100.2688

				36.66		100.2688

				36.67		100.2688

				36.69		100.2688

				36.7		100.2688

				36.72		100.2688

				36.73		100.2688

				36.75		100.2688

				36.77		100.2688

				36.78		100.2688

				36.8		100.2688

				36.81		100.2688

				36.83		100.2688

				36.84		100.2688

				36.86		100.2688

				36.88		100.2688

				36.89		100.2688

				36.91		100.2748

				36.92		100.2748

				36.94		100.2748

				36.96		100.2748

				36.97		100.2748

				36.99		100.2748

				37		100.2748

				37.02		100.2748

				37.04		100.2748

				37.05		100.2748

				37.07		100.2748

				37.08		100.2748

				37.1		100.2748

				37.11		100.2748

				37.13		100.2748

				37.15		100.2748

				37.16		100.2748

				37.18		100.2748

				37.19		100.2748

				37.21		100.2748

				37.23		100.2748

				37.24		100.2748

				37.26		100.2748

				37.28		100.2748

				37.29		100.2748

				37.31		100.2748

				37.32		100.2748

				37.34		100.2808

				37.36		100.2808

				37.37		100.2808

				37.39		100.2808

				37.4		100.2808

				37.42		100.2808

				37.44		100.2808

				37.45		100.2808

				37.47		100.2808

				37.48		100.2808

				37.5		100.2808

				37.52		100.2808

				37.53		100.2808

				37.55		100.2808

				37.57		100.2808

				37.58		100.2808

				37.6		100.2808

				37.61		100.2808

				37.63		100.2808

				37.65		100.2808

				37.66		100.2808

				37.68		100.2808

				37.7		100.2808

				37.71		100.2867

				37.73		100.2867

				37.74		100.2867

				37.76		100.2867

				37.78		100.2867

				37.79		100.2867

				37.81		100.2867

				37.83		100.2867

				37.84		100.2867

				37.86		100.2867

				37.88		100.2867

				37.89		100.2867

				37.91		100.2867

				37.93		100.2867

				37.94		100.2867

				37.96		100.2867

				37.97		100.2867

				37.99		100.2867

				38.01		100.2867

				38.02		100.2867

				38.04		100.2867

				38.06		100.2867

				38.07		100.2867

				38.09		100.2867

				38.11		100.2867

				38.12		100.2867

				38.14		100.2867

				38.16		100.2867

				38.17		100.2867

				38.19		100.2927

				38.21		100.2927

				38.22		100.2927

				38.24		100.2927

				38.26		100.2927

				38.27		100.2927

				38.29		100.2927

				38.31		100.2927

				38.32		100.2927

				38.34		100.2927

				38.36		100.2927

				38.37		100.2927

				38.39		100.2927

				38.41		100.2927

				38.42		100.2927

				38.44		100.2927

				38.46		100.2927

				38.47		100.2927

				38.49		100.2927

				38.51		100.2927

				38.52		100.2927

				38.54		100.2927

				38.56		100.2927

				38.57		100.2927

				38.59		100.2927

				38.61		100.2927

				38.62		100.2927

				38.64		100.2987

				38.66		100.2927

				38.67		100.2927

				38.69		100.2927

				38.71		100.2987

				38.72		100.2987

				38.74		100.2987

				38.76		100.2987

				38.78		100.2987

				38.79		100.2987

				38.81		100.2987

				38.83		100.2987

				38.84		100.2987

				38.86		100.2987

				38.88		100.2987

				38.89		100.2987

				38.91		100.2987

				38.93		100.2987

				38.94		100.2987

				38.96		100.2987

				38.98		100.2987

				39		100.2987

				39.01		100.2987

				39.03		100.2987

				39.05		100.2987

				39.06		100.2987

				39.08		100.2987

				39.1		100.2987

				39.11		100.2987

				39.13		100.2987

				39.15		100.2987

				39.17		100.2987

				39.18		100.2987

				39.2		100.2987

				39.22		100.2987

				39.23		100.2987

				39.25		100.2987

				39.27		100.2987

				39.29		100.2987

				39.3		100.2987

				39.32		100.2987

				39.34		100.2987

				39.35		100.2987

				39.37		100.2987

				39.39		100.2987

				39.41		100.2987

				39.42		100.2987

				39.44		100.2987

				39.46		100.2987

				39.47		100.2987

				39.49		100.2987

				39.51		100.2987

				39.53		100.2987

				39.54		100.2987

				39.56		100.2987

				39.58		100.2987

				39.59		100.2987

				39.61		100.2987

				39.63		100.2987

				39.65		100.2987

				39.66		100.2987

				39.68		100.2987

				39.7		100.2987

				39.72		100.2987

				39.73		100.2987

				39.75		100.2987

				39.77		100.2987

				39.79		100.2987

				39.8		100.2987

				39.82		100.2987

				39.84		100.2987

				39.85		100.3047

				39.87		100.2987

				39.89		100.3047

				39.91		100.2987

				39.92		100.3047

				39.94		100.3047

				39.96		100.3047

				39.98		100.3047

				39.99		100.3047

				40.01		100.3047

				40.03		100.3047

				40.05		100.3047

				40.06		100.3047

				40.08		100.3047

				40.1		100.3047

				40.12		100.3047

				40.13		100.3047

				40.15		100.3047

				40.17		100.3047

				40.19		100.3047

				40.2		100.3047

				40.22		100.3106

				40.24		100.3106

				40.26		100.3047

				40.27		100.3106

				40.29		100.3106

				40.31		100.3106

				40.33		100.3106

				40.34		100.3106

				40.36		100.3106

				40.38		100.3106

				40.4		100.3106

				40.41		100.3106

				40.43		100.3106

				40.45		100.3106

				40.47		100.3106

				40.48		100.3106

				40.5		100.3106

				40.52		100.3106

				40.54		100.3106

				40.56		100.3106

				40.57		100.3106

				40.59		100.3106

				40.61		100.3106

				40.63		100.3106

				40.64		100.3106

				40.66		100.3106

				40.68		100.3106

				40.7		100.3106

				40.71		100.3106

				40.73		100.3106

				40.75		100.3166

				40.77		100.3166

				40.79		100.3166

				40.8		100.3166

				40.82		100.3166

				40.84		100.3166

				40.86		100.3106

				40.87		100.3106

				40.89		100.3106

				40.91		100.3106

				40.93		100.3106

				40.95		100.3106

				40.96		100.3166

				40.98		100.3166

				41		100.3166

				41.02		100.3166

				41.03		100.3166

				41.05		100.3166

				41.07		100.3166

				41.09		100.3166

				41.11		100.3166

				41.12		100.3166

				41.14		100.3166

				41.16		100.3166

				41.18		100.3166

				41.2		100.3166

				41.21		100.3226

				41.23		100.3226

				41.25		100.3226

				41.27		100.3226

				41.29		100.3226

				41.3		100.3226

				41.32		100.3226

				41.34		100.3226

				41.36		100.3226

				41.37		100.3226

				41.39		100.3226

				41.41		100.3226

				41.43		100.3226

				41.45		100.3226

				41.46		100.3226

				41.48		100.3226

				41.5		100.3226

				41.52		100.3226

				41.54		100.3286

				41.55		100.3286

				41.57		100.3286

				41.59		100.3286

				41.61		100.3286

				41.63		100.3286

				41.65		100.3286

				41.66		100.3286

				41.68		100.3286

				41.7		100.3286

				41.72		100.3286

				41.74		100.3286

				41.75		100.3286

				41.77		100.3286

				41.79		100.3286

				41.81		100.3286

				41.83		100.3286

				41.84		100.3286

				41.86		100.3286

				41.88		100.3286

				41.9		100.3286

				41.92		100.3286

				41.93		100.3286

				41.95		100.3286

				41.97		100.3286

				41.99		100.3286

				42.01		100.3345

				42.03		100.3345

				42.04		100.3345

				42.06		100.3345

				42.08		100.3345

				42.1		100.3345

				42.12		100.3345

				42.13		100.3345

				42.15		100.3345

				42.17		100.3345

				42.19		100.3345

				42.21		100.3345

				42.23		100.3345

				42.24		100.3345

				42.26		100.3345

				42.28		100.3345

				42.3		100.3345

				42.32		100.3345

				42.34		100.3405

				42.35		100.3345

				42.37		100.3405

				42.39		100.3405

				42.41		100.3405

				42.43		100.3405

				42.44		100.3405

				42.46		100.3405

				42.48		100.3405

				42.5		100.3405

				42.52		100.3405

				42.54		100.3405

				42.55		100.3405

				42.57		100.3405

				42.59		100.3405

				42.61		100.3405

				42.63		100.3405

				42.65		100.3405

				42.66		100.3405

				42.68		100.3465

				42.7		100.3465

				42.72		100.3465

				42.74		100.3465

				42.76		100.3465

				42.78		100.3465

				42.79		100.3465

				42.81		100.3465

				42.83		100.3465

				42.85		100.3465

				42.87		100.3465

				42.89		100.3465

				42.9		100.3465

				42.92		100.3465

				42.94		100.3465

				42.96		100.3465

				42.98		100.3465

				43		100.3465

				43.01		100.3465

				43.03		100.3465

				43.05		100.3465

				43.07		100.3465

				43.09		100.3465

				43.11		100.3465

				43.13		100.3465

				43.14		100.3465

				43.16		100.3465

				43.18		100.3465

				43.2		100.3465

				43.22		100.3465

				43.24		100.3465

				43.26		100.3465

				43.27		100.3465

				43.29		100.3465

				43.31		100.3465

				43.33		100.3465

				43.35		100.3465

				43.37		100.3465

				43.39		100.3465

				43.4		100.3465

				43.42		100.3465

				43.44		100.3465

				43.46		100.3465

				43.48		100.3465

				43.5		100.3465

				43.52		100.3465

				43.53		100.3465

				43.55		100.3465

				43.57		100.3465

				43.59		100.3465

				43.61		100.3465

				43.63		100.3465

				43.65		100.3465

				43.66		100.3465

				43.68		100.3465

				43.7		100.3465

				43.72		100.3465

				43.74		100.3465

				43.76		100.3465

				43.78		100.3465

				43.8		100.3465

				43.81		100.3465

				43.83		100.3465

				43.85		100.3465

				43.87		100.3465

				43.89		100.3465

				43.91		100.3465

				43.93		100.3465

				43.95		100.3465

				43.96		100.3465

				43.98		100.3465

				44		100.3465

				44.02		100.3465

				44.04		100.3465

				44.06		100.3465

				44.08		100.3465

				44.1		100.3465

				44.11		100.3465

				44.13		100.3465

				44.15		100.3465

				44.17		100.3465

				44.19		100.3465

				44.21		100.3465

				44.23		100.3465

				44.25		100.3465

				44.26		100.3465

				44.28		100.3465

				44.3		100.3465

				44.32		100.3465

				44.34		100.3465

				44.36		100.3465

				44.38		100.3524

				44.4		100.3465

				44.41		100.3465

				44.43		100.3465

				44.45		100.3524

				44.47		100.3524

				44.49		100.3524

				44.51		100.3524

				44.53		100.3524

				44.55		100.3524

				44.57		100.3524

				44.58		100.3524

				44.6		100.3524

				44.62		100.3524

				44.64		100.3524

				44.66		100.3524

				44.68		100.3524

				44.7		100.3524

				44.72		100.3524

				44.74		100.3524

				44.75		100.3524

				44.77		100.3524

				44.79		100.3524

				44.81		100.3524

				44.83		100.3524

				44.85		100.3524

				44.87		100.3524

				44.89		100.3524

				44.91		100.3524

				44.93		100.3524

				44.94		100.3524

				44.96		100.3524

				44.98		100.3524

				45		100.3524

				45.02		100.3524

				45.04		100.3524

				45.06		100.3524

				45.08		100.3524

				45.1		100.3524

				45.12		100.3524

				45.13		100.3524

				45.15		100.3524

				45.17		100.3524

				45.19		100.3524

				45.21		100.3584

				45.23		100.3584

				45.25		100.3584

				45.27		100.3584

				45.29		100.3584

				45.31		100.3584

				45.32		100.3584

				45.34		100.3584

				45.36		100.3584

				45.38		100.3584

				45.4		100.3584

				45.42		100.3584

				45.44		100.3584

				45.46		100.3584

				45.48		100.3584

				45.5		100.3584

				45.52		100.3584

				45.53		100.3584

				45.55		100.3584

				45.57		100.3584

				45.59		100.3584

				45.61		100.3584

				45.63		100.3584

				45.65		100.3584

				45.67		100.3584

				45.69		100.3584

				45.71		100.3584

				45.73		100.3584

				45.74		100.3584

				45.76		100.3584

				45.78		100.3584

				45.8		100.3584

				45.82		100.3584

				45.84		100.3584

				45.86		100.3584

				45.88		100.3584

				45.9		100.3584

				45.92		100.3584

				45.94		100.3584

				45.96		100.3584

				45.97		100.3584

				45.99		100.3584

				46.01		100.3584

				46.03		100.3644

				46.05		100.3644

				46.07		100.3644

				46.09		100.3644

				46.11		100.3644

				46.13		100.3644

				46.15		100.3644

				46.17		100.3644

				46.19		100.3644

				46.2		100.3644

				46.22		100.3644

				46.24		100.3644

				46.26		100.3644

				46.28		100.3644

				46.3		100.3644

				46.32		100.3644

				46.34		100.3644

				46.36		100.3584

				46.38		100.3584

				46.4		100.3584

				46.42		100.3584

				46.44		100.3584

				46.46		100.3584

				46.47		100.3584

				46.49		100.3584

				46.51		100.3584

				46.53		100.3584

				46.55		100.3584

				46.57		100.3584

				46.59		100.3584

				46.61		100.3584

				46.63		100.3584

				46.65		100.3584

				46.67		100.3584

				46.69		100.3584

				46.71		100.3584

				46.73		100.3584

				46.74		100.3584

				46.76		100.3584

				46.78		100.3584

				46.8		100.3584

				46.82		100.3584

				46.84		100.3584

				46.86		100.3584

				46.88		100.3584

				46.9		100.3584

				46.92		100.3584

				46.94		100.3584

				46.96		100.3584

				46.98		100.3584

				47		100.3584

				47.02		100.3644

				47.03		100.3584

				47.05		100.3644

				47.07		100.3584

				47.09		100.3584

				47.11		100.3584

				47.13		100.3584

				47.15		100.3584

				47.17		100.3584

				47.19		100.3584

				47.21		100.3584

				47.23		100.3584

				47.25		100.3584

				47.27		100.3584

				47.29		100.3584

				47.31		100.3644

				47.33		100.3644

				47.35		100.3644

				47.36		100.3644

				47.38		100.3644

				47.4		100.3644

				47.42		100.3644

				47.44		100.3644

				47.46		100.3644

				47.48		100.3644

				47.5		100.3584

				47.52		100.3644

				47.54		100.3644

				47.56		100.3644

				47.58		100.3704

				47.6		100.3704

				47.62		100.3644

				47.64		100.3704

				47.66		100.3644

				47.68		100.3644

				47.7		100.3644

				47.72		100.3644

				47.74		100.3704

				47.75		100.3704

				47.77		100.3704

				47.79		100.3704

				47.81		100.3704

				47.83		100.3704

				47.85		100.3704

				47.87		100.3704

				47.89		100.3704

				47.91		100.3704

				47.93		100.3704

				47.95		100.3704

				47.97		100.3704

				47.99		100.3704

				48.01		100.3704

				48.03		100.3704

				48.05		100.3704

				48.07		100.3763

				48.09		100.3763

				48.11		100.3763

				48.13		100.3763

				48.15		100.3763

				48.17		100.3763

				48.18		100.3763

				48.2		100.3763

				48.22		100.3763

				48.24		100.3763

				48.26		100.3763

				48.28		100.3763

				48.3		100.3763

				48.32		100.3763

				48.34		100.3763

				48.36		100.3763

				48.38		100.3763

				48.4		100.3823

				48.42		100.3823

				48.44		100.3823

				48.46		100.3823

				48.48		100.3823

				48.5		100.3823

				48.52		100.3823

				48.54		100.3823

				48.56		100.3823

				48.58		100.3883

				48.6		100.3823

				48.62		100.3883

				48.64		100.3883

				48.66		100.3883

				48.68		100.3883

				48.69		100.3883

				48.71		100.3883

				48.73		100.3883

				48.75		100.3823

				48.77		100.3823

				48.79		100.3823

				48.81		100.3823

				48.83		100.3823

				48.85		100.3763

				48.87		100.3763

				48.89		100.3823

				48.91		100.3823

				48.93		100.3823

				48.95		100.3823

				48.97		100.3584

				48.99		100.3584

				49.01		100.3584

				49.03		100.3584

				49.05		100.3584

				49.07		100.3524

				49.09		100.3524

				49.11		100.3524

				49.13		100.3584

				49.15		100.3524

				49.17		100.3465

				49.19		100.3465

				49.21		100.3465

				49.23		100.3465

				49.25		100.3465

				49.27		100.3524

				49.29		100.3465

				49.31		100.3465

				49.33		100.3465

				49.34		100.3465

				49.36		100.3465

				49.38		100.3465

				49.4		100.3465

				49.42		100.3465

				49.44		100.3524

				49.46		100.3524

				49.48		100.3524

				49.5		100.3524

				49.52		100.3524

				49.54		100.3584

				49.56		100.3584

				49.58		100.3584

				49.6		100.3644

				49.62		100.3704

				49.64		100.3763

				49.66		100.3883

				49.68		100.3883

				49.7		100.3943

				49.72		100.3943

				49.74		100.3943

				49.76		100.3943

				49.78		100.3943

				49.8		100.3943

				49.82		100.3943

				49.84		100.3943

				49.86		100.3943

				49.88		100.3943

				49.9		100.3883

				49.92		100.3883

				49.94		100.3943

				49.96		100.3943

				49.98		100.3943

				50		100.3943

				50.02		100.3943

				50.04		100.3943

				50.06		100.3943

				50.08		100.3943

				50.1		100.3943

				50.12		100.3943

				50.14		100.3943

				50.16		100.3943

				50.18		100.3883

				50.2		100.4062

				50.22		100.448

				50.24		100.454

				50.26		100.46

				50.28		100.4659

				50.3		100.4659

				50.32		100.4719

				50.34		100.4779

				50.36		100.4779

				50.38		100.4779

				50.4		100.4779

				50.42		100.4719

				50.43		100.4659

				50.45		100.46

				50.47		100.46

				50.49		100.454

				50.51		100.454

				50.53		100.448

				50.55		100.448

				50.57		100.4421

				50.59		100.4421

				50.61		100.4361

				50.63		100.4361

				50.65		100.4361

				50.67		100.4361

				50.69		100.4301

				50.71		100.4301

				50.73		100.4301

				50.75		100.4301

				50.77		100.4301

				50.79		100.4301

				50.81		100.4361

				50.83		100.4301

				50.85		100.4301

				50.87		100.4361

				50.89		100.4361

				50.91		100.4301

				50.93		100.4301

				50.95		100.4361

				50.97		100.4361

				50.99		100.4301

				51.01		100.4301

				51.03		100.4301

				51.05		100.4301

				51.07		100.4301

				51.09		100.4301

				51.11		100.4301

				51.13		100.4241

				51.15		100.4241

				51.17		100.4241

				51.19		100.4241

				51.21		100.4182

				51.23		100.4122

				51.25		100.4122

				51.27		100.4122

				51.29		100.4122

				51.31		100.4122

				51.33		100.4122

				51.35		100.4062

				51.37		100.4062

				51.39		100.4002

				51.41		100.3943

				51.43		100.3943

				51.45		100.3943

				51.47		100.3943

				51.49		100.3943

				51.51		100.3943

				51.53		100.3943

				51.55		100.3943

				51.57		100.3943

				51.59		100.3943

				51.61		100.3943

				51.63		100.3943

				51.65		100.3943

				51.67		100.3943

				51.69		100.3943

				51.71		100.3943

				51.73		100.3943

				51.75		100.3943

				51.77		100.3943

				51.79		100.3943

				51.81		100.4002

				51.83		100.4002

				51.85		100.4002

				51.87		100.4002

				51.89		100.4002

				51.91		100.4002

				51.93		100.4002

				51.95		100.4002

				51.97		100.4002

				51.99		100.4002

				52.01		100.4002

				52.03		100.4002

				52.05		100.4002

				52.07		100.4002

				52.09		100.4002

				52.11		100.4002

				52.13		100.4002

				52.16		100.4002

				52.18		100.4002

				52.2		100.4062

				52.22		100.4062

				52.24		100.4062

				52.26		100.4062

				52.28		100.4062

				52.3		100.4062

				52.32		100.4062

				52.34		100.4062

				52.36		100.4062

				52.38		100.4062

				52.4		100.4062

				52.42		100.4062

				52.44		100.4062

				52.46		100.4062

				52.48		100.4062

				52.5		100.4062

				52.52		100.4062

				52.54		100.4062

				52.56		100.4062

				52.58		100.4062

				52.6		100.4062

				52.62		100.4062

				52.64		100.4062

				52.66		100.4062

				52.68		100.4062

				52.7		100.4062

				52.72		100.4062

				52.74		100.4062

				52.76		100.4062

				52.78		100.4062

				52.8		100.4062

				52.82		100.4062

				52.84		100.4062

				52.86		100.4062

				52.88		100.4062

				52.9		100.4062

				52.92		100.4062

				52.94		100.4062

				52.96		100.4062

				52.98		100.4062

				53		100.4122

				53.02		100.4122

				53.04		100.4122

				53.06		100.4122

				53.08		100.4122

				53.1		100.4122

				53.12		100.4122

				53.14		100.4122

				53.16		100.4122

				53.18		100.4122

				53.2		100.4122

				53.22		100.4122

				53.24		100.4122

				53.26		100.4122

				53.28		100.4122

				53.3		100.4122

				53.32		100.4122

				53.34		100.4122

				53.36		100.4062

				53.38		100.4122

				53.4		100.4122

				53.42		100.4122

				53.44		100.4122

				53.46		100.4122

				53.49		100.4122

				53.51		100.4122

				53.53		100.4122

				53.55		100.4122

				53.57		100.4122

				53.59		100.4122

				53.61		100.4122

				53.63		100.4122

				53.65		100.4122

				53.67		100.4122

				53.69		100.4122

				53.71		100.4122

				53.73		100.4122

				53.75		100.4122

				53.77		100.4122

				53.79		100.4122

				53.81		100.4122

				53.83		100.4122

				53.85		100.4122

				53.87		100.4122

				53.89		100.4122

				53.91		100.4122

				53.93		100.4122

				53.95		100.4122

				53.97		100.4122

				53.99		100.4122

				54.01		100.4122

				54.03		100.4122

				54.05		100.4122

				54.07		100.4122

				54.09		100.4122

				54.11		100.4122

				54.13		100.4122

				54.15		100.4122

				54.17		100.4122

				54.19		100.4122

				54.21		100.4122

				54.23		100.4122

				54.25		100.4122

				54.27		100.4122

				54.3		100.4122

				54.32		100.4122

				54.34		100.4122

				54.36		100.4122

				54.38		100.4122

				54.4		100.4122

				54.42		100.4122

				54.44		100.4122

				54.46		100.4122

				54.48		100.4122

				54.5		100.4122

				54.52		100.4122

				54.54		100.4122

				54.56		100.4122

				54.58		100.4122

				54.6		100.4122

				54.62		100.4122

				54.64		100.4122

				54.66		100.4122

				54.68		100.4122

				54.7		100.4122

				54.72		100.4122

				54.74		100.4122

				54.76		100.4122

				54.78		100.4122

				54.8		100.4122

				54.82		100.4122

				54.84		100.4122

				54.86		100.4122

				54.88		100.4122

				54.9		100.4122

				54.92		100.4122

				54.95		100.4122

				54.97		100.4122

				54.99		100.4122

				55.01		100.4062

				55.03		100.4122

				55.05		100.4122

				55.07		100.4062

				55.09		100.4122

				55.11		100.4122

				55.13		100.4122

				55.15		100.4122

				55.17		100.4122

				55.19		100.4062

				55.21		100.4062

				55.23		100.4062

				55.25		100.4062

				55.27		100.4062

				55.29		100.4062

				55.31		100.4062

				55.33		100.4122

				55.35		100.4122

				55.37		100.4122

				55.39		100.4122

				55.41		100.4062

				55.43		100.4062

				55.45		100.4062

				55.47		100.4062

				55.5		100.4062

				55.52		100.4062

				55.54		100.4062

				55.56		100.4122

				55.58		100.4122

				55.6		100.4122

				55.62		100.4122

				55.64		100.4122

				55.66		100.4122

				55.68		100.4122

				55.7		100.4122

				55.72		100.4122

				55.74		100.4122

				55.76		100.4122

				55.78		100.4122

				55.8		100.4122

				55.82		100.4122

				55.84		100.4122

				55.86		100.4122

				55.88		100.4122

				55.9		100.4122

				55.92		100.4122

				55.94		100.4062

				55.96		100.4062

				55.98		100.4062

				56.01		100.4062

				56.03		100.4062

				56.05		100.4062

				56.07		100.4062

				56.09		100.4062

				56.11		100.4062

				56.13		100.4062

				56.15		100.4062

				56.17		100.4062

				56.19		100.4062

				56.21		100.4062

				56.23		100.4062

				56.25		100.4062

				56.27		100.4062

				56.29		100.4062

				56.31		100.4062

				56.33		100.4062

				56.35		100.4062

				56.37		100.4062

				56.39		100.4062

				56.41		100.4062

				56.43		100.4062

				56.45		100.4062

				56.48		100.4062

				56.5		100.4062

				56.52		100.4062

				56.54		100.4062

				56.56		100.4062

				56.58		100.4062

				56.6		100.4062

				56.62		100.4062

				56.64		100.4062

				56.66		100.4062

				56.68		100.4062

				56.7		100.4062

				56.72		100.4062

				56.74		100.4062

				56.76		100.4062

				56.78		100.4062

				56.8		100.4062

				56.82		100.4062

				56.84		100.4062

				56.86		100.4062

				56.88		100.4062

				56.91		100.4062

				56.93		100.4062

				56.95		100.4062

				56.97		100.4062

				56.99		100.4062

				57.01		100.4062

				57.03		100.4062

				57.05		100.4062

				57.07		100.4062

				57.09		100.4062

				57.11		100.4062

				57.13		100.4062

				57.15		100.4062

				57.17		100.4062

				57.19		100.4062

				57.21		100.4062

				57.23		100.4062

				57.25		100.4062

				57.27		100.4062

				57.3		100.4062

				57.32		100.4062

				57.34		100.4062

				57.36		100.4062

				57.38		100.4062

				57.4		100.4062

				57.42		100.4062

				57.44		100.4062

				57.46		100.4062

				57.48		100.4062

				57.5		100.4062

				57.52		100.4062

				57.54		100.4062

				57.56		100.4062

				57.58		100.4062

				57.6		100.4062

				57.62		100.4062

				57.64		100.4062

				57.66		100.4062

				57.69		100.4062

				57.71		100.4062

				57.73		100.4062

				57.75		100.4062

				57.77		100.4062

				57.79		100.4062

				57.81		100.4122

				57.83		100.4062

				57.85		100.4062

				57.87		100.4062

				57.89		100.4122

				57.91		100.4122

				57.93		100.4122

				57.95		100.4122

				57.97		100.4122

				57.99		100.4122

				58.01		100.4122

				58.03		100.4122

				58.06		100.4122

				58.08		100.4122

				58.1		100.4122

				58.12		100.4122

				58.14		100.4122

				58.16		100.4122

				58.18		100.4122

				58.2		100.4122

				58.22		100.4122

				58.24		100.4122

				58.26		100.4122

				58.28		100.4122

				58.3		100.4122

				58.32		100.4122

				58.34		100.4122

				58.36		100.4122

				58.38		100.4122

				58.4		100.4122

				58.43		100.4122

				58.45		100.4122

				58.47		100.4122

				58.49		100.4122

				58.51		100.4122

				58.53		100.4122

				58.55		100.4122

				58.57		100.4122

				58.59		100.4122

				58.61		100.4122

				58.63		100.4122

				58.65		100.4122

				58.67		100.4122

				58.69		100.4122

				58.71		100.4122

				58.73		100.4122

				58.75		100.4122

				58.78		100.4182

				58.8		100.4122

				58.82		100.4182

				58.84		100.4122

				58.86		100.4182

				58.88		100.4122

				58.9		100.4182

				58.92		100.4182

				58.94		100.4182

				58.96		100.4182

				58.98		100.4182

				59		100.4182

				59.02		100.4182

				59.04		100.4182

				59.06		100.4182

				59.08		100.4182

				59.11		100.4182

				59.13		100.4182

				59.15		100.4182

				59.17		100.4182

				59.19		100.4182

				59.21		100.4182

				59.23		100.4241

				59.25		100.4182

				59.27		100.4241

				59.29		100.4241

				59.31		100.4241

				59.33		100.4241

				59.35		100.4241

				59.37		100.4241

				59.39		100.4241

				59.41		100.4241

				59.43		100.4241

				59.46		100.4241

				59.48		100.4241

				59.5		100.4241

				59.52		100.4301

				59.54		100.4241

				59.56		100.4301

				59.58		100.4241

				59.6		100.4301

				59.62		100.4301

				59.64		100.4301

				59.66		100.4301

				59.68		100.4301

				59.7		100.4301

				59.72		100.4301

				59.74		100.4301

				59.76		100.4301

				59.79		100.4301

				59.81		100.4301

				59.83		100.4301

				59.85		100.4301

				59.87		100.4301

				59.89		100.4301

				59.91		100.4301

				59.93		100.4301

				59.95		100.4301

				59.97		100.4301

				59.99		100.4301

				60.01		100.4361

				60.03		100.4301

				60.05		100.4361

				60.07		100.4361

				60.09		100.4361

				60.12		100.4361

				60.14		100.4361

				60.16		100.4361

				60.18		100.4361

				60.2		100.4361

				60.22		100.4361

				60.24		100.4361

				60.26		100.4361

				60.28		100.4361

				60.3		100.4361

				60.32		100.4361

				60.34		100.4361

				60.36		100.4421

				60.38		100.4421

				60.4		100.4421

				60.42		100.4421

				60.45		100.4421

				60.47		100.4421

				60.49		100.4421

				60.51		100.4421

				60.53		100.4421

				60.55		100.4421

				60.57		100.4421

				60.59		100.4421

				60.61		100.4421

				60.63		100.4421

				60.65		100.448

				60.67		100.448

				60.69		100.448

				60.71		100.448

				60.73		100.448

				60.75		100.448

				60.77		100.448

				60.8		100.448

				60.82		100.448

				60.84		100.448

				60.86		100.448

				60.88		100.448

				60.9		100.448

				60.92		100.448

				60.94		100.448

				60.96		100.454

				60.98		100.448

				61		100.454

				61.02		100.454

				61.04		100.454

				61.06		100.454

				61.08		100.454

				61.1		100.454

				61.12		100.454

				61.15		100.454

				61.17		100.454

				61.19		100.454

				61.21		100.454

				61.23		100.46

				61.25		100.46

				61.27		100.46

				61.29		100.46

				61.31		100.46

				61.33		100.46

				61.35		100.46

				61.37		100.46

				61.39		100.46

				61.41		100.46

				61.43		100.46

				61.45		100.46

				61.47		100.46

				61.5		100.46

				61.52		100.46

				61.54		100.46

				61.56		100.46

				61.58		100.46

				61.6		100.46

				61.62		100.46

				61.64		100.46

				61.66		100.46

				61.68		100.46

				61.7		100.46

				61.72		100.46

				61.74		100.46

				61.76		100.46

				61.78		100.46

				61.8		100.46

				61.82		100.46

				61.84		100.46

				61.87		100.4659

				61.89		100.46

				61.91		100.46

				61.93		100.46

				61.95		100.46

				61.97		100.46

				61.99		100.4659

				62.01		100.4659

				62.03		100.4659

				62.05		100.4659

				62.07		100.4659

				62.09		100.4659

				62.11		100.4659

				62.13		100.4659

				62.15		100.4659

				62.17		100.4659

				62.19		100.4659

				62.22		100.4659

				62.24		100.4659

				62.26		100.4659

				62.28		100.4659

				62.3		100.4659

				62.32		100.4659

				62.34		100.4659

				62.36		100.4659

				62.38		100.4659

				62.4		100.4659

				62.42		100.4659

				62.44		100.4659

				62.46		100.4659

				62.48		100.4659

				62.5		100.4659

				62.52		100.4659

				62.54		100.4659

				62.56		100.4659

				62.59		100.4659

				62.61		100.4659

				62.63		100.4659

				62.65		100.4659

				62.67		100.4659

				62.69		100.4659

				62.71		100.4659

				62.73		100.4659

				62.75		100.4659

				62.77		100.4659

				62.79		100.4659

				62.81		100.4659

				62.83		100.4659

				62.85		100.4719

				62.87		100.4659

				62.89		100.4659

				62.91		100.4659

				62.94		100.4659

				62.96		100.4659

				62.98		100.4659

				63		100.4659

				63.02		100.4659

				63.04		100.4659

				63.06		100.4659

				63.08		100.4659

				63.1		100.4659

				63.12		100.4659

				63.14		100.4659

				63.16		100.4659

				63.18		100.4659

				63.2		100.4659

				63.22		100.4659

				63.24		100.4659

				63.26		100.46

				63.28		100.46

				63.31		100.46

				63.33		100.46

				63.35		100.46

				63.37		100.46

				63.39		100.46

				63.41		100.46

				63.43		100.4659

				63.45		100.46

				63.47		100.46

				63.49		100.46

				63.51		100.4659

				63.53		100.4659

				63.55		100.4659

				63.57		100.4659

				63.59		100.4659

				63.61		100.4659

				63.63		100.4659

				63.66		100.4659

				63.68		100.4659

				63.7		100.4659

				63.72		100.4659

				63.74		100.4659

				63.76		100.4659

				63.78		100.4659

				63.8		100.4659

				63.82		100.4659

				63.84		100.4659

				63.86		100.4659

				63.88		100.4659

				63.9		100.4659

				63.92		100.4659

				63.94		100.4659

				63.96		100.4659

				63.98		100.4659

				64		100.4659

				64.03		100.4659

				64.05		100.4659

				64.07		100.4659

				64.09		100.4659

				64.11		100.4659

				64.13		100.4659

				64.15		100.4659

				64.17		100.4659

				64.19		100.4659

				64.21		100.4659

				64.23		100.4659

				64.25		100.4659

				64.27		100.4659

				64.29		100.4659

				64.31		100.4659

				64.33		100.4659

				64.35		100.4659

				64.38		100.4659

				64.4		100.4659

				64.42		100.4659

				64.44		100.4659

				64.46		100.4659

				64.48		100.4659

				64.5		100.4659

				64.52		100.4659

				64.54		100.4659

				64.56		100.4659

				64.58		100.4659

				64.6		100.4659

				64.62		100.4659

				64.64		100.4659

				64.66		100.4659

				64.68		100.4659

				64.71		100.4659

				64.73		100.4659

				64.75		100.4659

				64.77		100.4659

				64.79		100.4659

				64.81		100.4659

				64.83		100.4659

				64.85		100.4659

				64.87		100.4659

				64.89		100.4659

				64.91		100.4659

				64.93		100.4659

				64.95		100.4659

				64.97		100.4659

				64.99		100.4659

				65.01		100.4659

				65.04		100.4659

				65.06		100.4659

				65.08		100.4659

				65.1		100.4659

				65.12		100.4659

				65.14		100.4659

				65.16		100.4659

				65.18		100.4659

				65.2		100.4659

				65.22		100.4659

				65.24		100.4659

				65.26		100.4659

				65.28		100.4659

				65.3		100.4659

				65.32		100.4659

				65.35		100.4719

				65.37		100.4719

				65.39		100.4719

				65.41		100.4719

				65.43		100.4719

				65.45		100.4719

				65.47		100.4719

				65.49		100.4719

				65.51		100.4719

				65.53		100.4719

				65.55		100.4719

				65.57		100.4719

				65.59		100.4719

				65.61		100.4719

				65.63		100.4719

				65.65		100.4719

				65.68		100.4719

				65.7		100.4719

				65.72		100.4719

				65.74		100.4719

				65.76		100.4719

				65.78		100.4719

				65.8		100.4719

				65.82		100.4719

				65.84		100.4719

				65.86		100.4719

				65.88		100.4719

				65.9		100.4719

				65.92		100.4719

				65.94		100.4719

				65.96		100.4719

				65.99		100.4719

				66.01		100.4719

				66.03		100.4719

				66.05		100.4719

				66.07		100.4719

				66.09		100.4719

				66.11		100.4719

				66.13		100.4719

				66.15		100.4719

				66.17		100.4719

				66.19		100.4719

				66.21		100.4719

				66.23		100.4719

				66.25		100.4719

				66.28		100.4719

				66.3		100.4719

				66.32		100.4719

				66.34		100.4719

				66.36		100.4719

				66.38		100.4719

				66.4		100.4719

				66.42		100.4719

				66.44		100.4719

				66.46		100.4719

				66.48		100.4719

				66.5		100.4719

				66.52		100.4719

				66.54		100.4719

				66.57		100.4719

				66.59		100.4719

				66.61		100.4719

				66.63		100.4719

				66.65		100.4719

				66.67		100.4719

				66.69		100.4719

				66.71		100.4719

				66.73		100.4719

				66.75		100.4659

				66.77		100.4659

				66.79		100.4659

				66.81		100.4659

				66.83		100.4659

				66.86		100.4659

				66.88		100.4659

				66.9		100.4659

				66.92		100.4659

				66.94		100.4659

				66.96		100.4659

				66.98		100.4659

				67		100.4659

				67.02		100.4659

				67.04		100.4659

				67.06		100.4659

				67.08		100.4659

				67.1		100.4659

				67.12		100.4659

				67.15		100.4659

				67.17		100.4659

				67.19		100.4659

				67.21		100.4659

				67.23		100.4659

				67.25		100.4659

				67.27		100.4659

				67.29		100.4659

				67.31		100.4659

				67.33		100.46

				67.35		100.4659

				67.37		100.46

				67.39		100.46

				67.42		100.4659

				67.44		100.4659

				67.46		100.4659

				67.48		100.4659

				67.5		100.4659

				67.52		100.4659

				67.54		100.4659

				67.56		100.4659

				67.58		100.4659

				67.6		100.4659

				67.62		100.4659

				67.64		100.4659

				67.66		100.4659

				67.69		100.4659

				67.71		100.4659

				67.73		100.4659

				67.75		100.4659

				67.77		100.4659

				67.79		100.4659

				67.81		100.4659

				67.83		100.4659

				67.85		100.4659

				67.87		100.4659

				67.89		100.4659

				67.91		100.4659

				67.93		100.4659

				67.96		100.4659

				67.98		100.4659

				68		100.4659

				68.02		100.4659

				68.04		100.4659

				68.06		100.4659

				68.08		100.4659

				68.1		100.4659

				68.12		100.4659

				68.14		100.4659

				68.16		100.4659

				68.18		100.4659

				68.2		100.4659

				68.23		100.4659

				68.25		100.4719

				68.27		100.4719

				68.29		100.4719

				68.31		100.4719

				68.33		100.4719

				68.35		100.4719

				68.37		100.4719

				68.39		100.4719

				68.41		100.4719

				68.43		100.4719

				68.45		100.4719

				68.48		100.4719

				68.5		100.4719

				68.52		100.4719

				68.54		100.4719

				68.56		100.4719

				68.58		100.4659

				68.6		100.4659

				68.62		100.4659

				68.64		100.4659

				68.66		100.4659

				68.68		100.4659

				68.7		100.4659

				68.72		100.4659

				68.75		100.4659

				68.77		100.4659

				68.79		100.4659

				68.81		100.4659

				68.83		100.4719

				68.85		100.4719

				68.87		100.4719

				68.89		100.4719

				68.91		100.4719

				68.93		100.4719

				68.95		100.4719

				68.97		100.4719

				69		100.4719

				69.02		100.4719

				69.04		100.4719

				69.06		100.4719

				69.08		100.4719

				69.1		100.4719

				69.12		100.4719

				69.14		100.4719

				69.16		100.4719

				69.18		100.4719

				69.2		100.4719

				69.22		100.4719

				69.25		100.4719

				69.27		100.4719

				69.29		100.4719

				69.31		100.4719

				69.33		100.4719

				69.35		100.4719

				69.37		100.4719

				69.39		100.4719

				69.41		100.4719

				69.43		100.4719

				69.45		100.4719

				69.48		100.4719

				69.5		100.4719

				69.52		100.4719

				69.54		100.4719

				69.56		100.4719

				69.58		100.4719

				69.6		100.4719

				69.62		100.4719

				69.64		100.4719

				69.66		100.4719

				69.68		100.4719

				69.7		100.4719

				69.73		100.4719

				69.75		100.4719

				69.77		100.4719

				69.79		100.4719

				69.81		100.4719

				69.83		100.4719

				69.85		100.4719

				69.87		100.4719

				69.89		100.4719

				69.91		100.4719

				69.93		100.4719

				69.96		100.4719

				69.98		100.4719

				70		100.4719

				70.02		100.4719

				70.04		100.4719

				70.06		100.4719

				70.08		100.4719

				70.1		100.4719

				70.12		100.4719

				70.14		100.4659

				70.16		100.4719

				70.18		100.4659

				70.21		100.4719

				70.23		100.4719

				70.25		100.4659

				70.27		100.4659

				70.29		100.4659

				70.31		100.4659

				70.33		100.4659

				70.35		100.4659

				70.37		100.4659

				70.39		100.4659

				70.41		100.4659

				70.44		100.4659

				70.46		100.4659

				70.48		100.4659

				70.5		100.4659

				70.52		100.4659

				70.54		100.4659

				70.56		100.4659

				70.58		100.4659

				70.6		100.4719

				70.62		100.4719

				70.64		100.4719

				70.67		100.4719

				70.69		100.4719

				70.71		100.4719

				70.73		100.4719

				70.75		100.4719

				70.77		100.4719

				70.79		100.4719

				70.81		100.4719

				70.83		100.4719

				70.85		100.4719

				70.87		100.4779

				70.9		100.4779

				70.92		100.4779

				70.94		100.4779

				70.96		100.4779

				70.98		100.4779

				71		100.4779

				71.02		100.4779

				71.04		100.4779

				71.06		100.4779

				71.08		100.4779

				71.1		100.4779

				71.13		100.4779

				71.15		100.4779

				71.17		100.4779

				71.19		100.4779

				71.21		100.4779

				71.23		100.4779

				71.25		100.4779

				71.27		100.4779

				71.29		100.4779

				71.31		100.4779

				71.33		100.4779

				71.36		100.4779

				71.38		100.4779

				71.4		100.4779

				71.42		100.4779

				71.44		100.4779

				71.46		100.4779

				71.48		100.4779

				71.5		100.4779

				71.52		100.4779

				71.54		100.4779

				71.56		100.4779

				71.59		100.4779

				71.61		100.4779

				71.63		100.4779

				71.65		100.4719

				71.67		100.4719

				71.69		100.4719

				71.71		100.4719

				71.73		100.4779

				71.75		100.4719

				71.77		100.4719

				71.79		100.4719

				71.82		100.4719

				71.84		100.4719

				71.86		100.4719

				71.88		100.4719

				71.9		100.4719

				71.92		100.4719

				71.94		100.4719

				71.96		100.4719

				71.98		100.4719

				72		100.4719

				72.03		100.4719

				72.05		100.4719

				72.07		100.4719

				72.09		100.4719

				72.11		100.4719

				72.13		100.4719

				72.15		100.4719

				72.17		100.4719

				72.19		100.4719

				72.21		100.4719

				72.24		100.4719

				72.26		100.4719

				72.28		100.4719

				72.3		100.4719

				72.32		100.4719

				72.34		100.4719

				72.36		100.4719

				72.38		100.4719

				72.4		100.4719

				72.42		100.4719

				72.44		100.4719

				72.47		100.4719

				72.49		100.4719

				72.51		100.4719

				72.53		100.4719

				72.55		100.4719

				72.57		100.4719

				72.59		100.4719

				72.61		100.4719

				72.63		100.4719

				72.65		100.4719

				72.68		100.4719

				72.7		100.4719

				72.72		100.4719

				72.74		100.4719

				72.76		100.4659

				72.78		100.4719

				72.8		100.4719

				72.82		100.4719

				72.84		100.4659

				72.86		100.4659

				72.89		100.4659

				72.91		100.4659

				72.93		100.4659

				72.95		100.4659

				72.97		100.4659

				72.99		100.4659

				73.01		100.4659

				73.03		100.4659

				73.05		100.4659

				73.07		100.4659

				73.1		100.4659

				73.12		100.4659

				73.14		100.4659

				73.16		100.4659

				73.18		100.4659

				73.2		100.4659

				73.22		100.4659

				73.24		100.4659

				73.26		100.4659

				73.28		100.4659

				73.3		100.4659

				73.33		100.4659

				73.35		100.4659

				73.37		100.4659

				73.39		100.4659

				73.41		100.4659

				73.43		100.4659

				73.45		100.4659

				73.47		100.4659

				73.49		100.4659

				73.51		100.4659

				73.54		100.4659

				73.56		100.4719

				73.58		100.4719

				73.6		100.4719

				73.62		100.4719

				73.64		100.4719

				73.66		100.4719

				73.68		100.4719

				73.7		100.4719

				73.72		100.4719

				73.75		100.4719

				73.77		100.4719

				73.79		100.4719

				73.81		100.4719

				73.83		100.4719

				73.85		100.4719

				73.87		100.4719

				73.89		100.4779

				73.91		100.4779

				73.93		100.4779

				73.96		100.4779

				73.98		100.4779

				74		100.4779

				74.02		100.4779

				74.04		100.4779

				74.06		100.4779

				74.08		100.4779

				74.1		100.4779

				74.12		100.4779

				74.14		100.4779

				74.17		100.4779

				74.19		100.4719

				74.21		100.4779

				74.23		100.4779

				74.25		100.4779

				74.27		100.4779

				74.29		100.4779

				74.31		100.4779

				74.33		100.4779

				74.35		100.4779

				74.38		100.4779

				74.4		100.4779

				74.42		100.4779

				74.44		100.4779

				74.46		100.4839

				74.48		100.4839

				74.5		100.4839

				74.52		100.4839

				74.54		100.4839

				74.56		100.4839

				74.59		100.4839

				74.61		100.4839

				74.63		100.4839

				74.65		100.4839

				74.67		100.4839

				74.69		100.4839

				74.71		100.4839

				74.73		100.4839

				74.75		100.4839

				74.77		100.4839

				74.8		100.4839

				74.82		100.4839

				74.84		100.4839

				74.86		100.4839

				74.88		100.4839

				74.9		100.4839

				74.92		100.4839

				74.94		100.4839

				74.96		100.4839

				74.98		100.4839

				75.01		100.4839

				75.03		100.4839

				75.05		100.4839

				75.07		100.4839

				75.09		100.4839

				75.11		100.4839

				75.13		100.4839

				75.15		100.4839

				75.17		100.4839

				75.19		100.4839

				75.22		100.4839

				75.24		100.4839

				75.26		100.4839

				75.28		100.4839

				75.3		100.4839

				75.32		100.4839

				75.34		100.4839

				75.36		100.4839

				75.38		100.4839

				75.4		100.4839

				75.43		100.4839

				75.45		100.4839

				75.47		100.4839

				75.49		100.4839

				75.51		100.4839

				75.53		100.4839

				75.55		100.4839

				75.57		100.4839

				75.59		100.4839

				75.62		100.4839

				75.64		100.4779

				75.66		100.4779

				75.68		100.4839

				75.7		100.4779

				75.72		100.4779

				75.74		100.4779

				75.76		100.4779

				75.78		100.4839

				75.8		100.4839

				75.83		100.4839

				75.85		100.4839

				75.87		100.4839

				75.89		100.4839

				75.91		100.4779

				75.93		100.4839

				75.95		100.4839

				75.97		100.4779

				75.99		100.4839

				76.01		100.4779

				76.04		100.4779

				76.06		100.4779

				76.08		100.4779

				76.1		100.4779

				76.12		100.4779

				76.14		100.4779

				76.16		100.4779

				76.18		100.4779

				76.2		100.4779

				76.22		100.4839

				76.25		100.4779

				76.27		100.4839

				76.29		100.4779

				76.31		100.4839

				76.33		100.4839

				76.35		100.4839

				76.37		100.4839

				76.39		100.4779

				76.41		100.4779

				76.43		100.4779

				76.46		100.4779

				76.48		100.4779

				76.5		100.4779

				76.52		100.4779

				76.54		100.4779

				76.56		100.4779

				76.58		100.4779

				76.6		100.4779

				76.62		100.4779

				76.65		100.4779

				76.67		100.4779

				76.69		100.4779

				76.71		100.4779

				76.73		100.4779

				76.75		100.4779

				76.77		100.4779

				76.79		100.4779

				76.81		100.4779

				76.83		100.4779

				76.86		100.4779

				76.88		100.4779

				76.9		100.4779

				76.92		100.4779

				76.94		100.4779

				76.96		100.4779

				76.98		100.4779

				77		100.4779

				77.02		100.4779

				77.05		100.4779

				77.07		100.4779

				77.09		100.4779

				77.11		100.4779

				77.13		100.4779

				77.15		100.4779

				77.17		100.4779

				77.19		100.4779

				77.21		100.4779

				77.23		100.4779

				77.26		100.4779

				77.28		100.4779

				77.3		100.4779

				77.32		100.4779

				77.34		100.4779

				77.36		100.4779

				77.38		100.4779

				77.4		100.4779

				77.42		100.4779

				77.44		100.4779

				77.47		100.4779

				77.49		100.4779

				77.51		100.4779

				77.53		100.4779

				77.55		100.4779

				77.57		100.4779

				77.59		100.4779

				77.61		100.4779

				77.63		100.4779

				77.66		100.4779

				77.68		100.4779

				77.7		100.4779

				77.72		100.4779

				77.74		100.4779

				77.76		100.4779

				77.78		100.4779

				77.8		100.4779

				77.82		100.4779

				77.84		100.4779

				77.87		100.4779

				77.89		100.4779

				77.91		100.4779

				77.93		100.4779

				77.95		100.4779

				77.97		100.4779

				77.99		100.4779

				78.01		100.4779

				78.03		100.4779

				78.05		100.4719

				78.08		100.4719

				78.1		100.4779

				78.12		100.4779

				78.14		100.4779

				78.16		100.4779

				78.18		100.4779

				78.2		100.4779

				78.22		100.4779

				78.24		100.4779

				78.27		100.4779

				78.29		100.4779

				78.31		100.4779

				78.33		100.4779

				78.35		100.4779

				78.37		100.4779

				78.39		100.4779

				78.41		100.4779

				78.43		100.4779

				78.45		100.4779

				78.48		100.4779

				78.5		100.4779

				78.52		100.4779

				78.54		100.4779

				78.56		100.4779

				78.58		100.4779

				78.6		100.4779

				78.62		100.4779

				78.64		100.4839

				78.67		100.4779

				78.69		100.4839

				78.71		100.4839

				78.73		100.4839

				78.75		100.4839

				78.77		100.4839

				78.79		100.4839

				78.81		100.4839

				78.83		100.4839

				78.85		100.4839

				78.88		100.4839

				78.9		100.4839

				78.92		100.4839

				78.94		100.4839

				78.96		100.4839

				78.98		100.4839

				79		100.4839

				79.02		100.4839

				79.04		100.4839

				79.07		100.4839

				79.09		100.4839

				79.11		100.4839

				79.13		100.4839

				79.15		100.4839

				79.17		100.4839

				79.19		100.4839

				79.21		100.4898

				79.23		100.4898

				79.25		100.4898

				79.28		100.4898

				79.3		100.4898

				79.32		100.4898

				79.34		100.4898

				79.36		100.4898

				79.38		100.4898

				79.4		100.4898

				79.42		100.4898

				79.44		100.4898

				79.47		100.4898

				79.49		100.4898

				79.51		100.4898

				79.53		100.4898

				79.55		100.4898

				79.57		100.4958

				79.59		100.4958

				79.61		100.4958

				79.63		100.4958

				79.65		100.4958

				79.68		100.4958

				79.7		100.4958

				79.72		100.4958

				79.74		100.4958

				79.76		100.4958

				79.78		100.4958

				79.8		100.4958

				79.82		100.4958

				79.84		100.4958

				79.87		100.4958

				79.89		100.5018

				79.91		100.4958

				79.93		100.5018

				79.95		100.5018

				79.97		100.5018

				79.99		100.5018

				80.01		100.5018

				80.03		100.5018

				80.06		100.5018

				80.08		100.5018

				80.1		100.5018

				80.12		100.5018

				80.14		100.5018

				80.16		100.5018

				80.18		100.5018

				80.2		100.5018

				80.22		100.5018

				80.24		100.5018

				80.27		100.5018

				80.29		100.5018

				80.31		100.5018

				80.33		100.5018

				80.35		100.5018

				80.37		100.5018

				80.39		100.5018

				80.41		100.5018

				80.43		100.5078

				80.46		100.5078

				80.48		100.5018

				80.5		100.5078

				80.52		100.5078

				80.54		100.5078

				80.56		100.5018

				80.58		100.5018

				80.6		100.5018

				80.62		100.5018

				80.64		100.5018

				80.67		100.5078

				80.69		100.5018

				80.71		100.5018

				80.73		100.5018

				80.75		100.5078

				80.77		100.5018

				80.79		100.5018

				80.81		100.5018

				80.83		100.5018

				80.86		100.5078

				80.88		100.5018

				80.9		100.5018

				80.92		100.5018

				80.94		100.5078

				80.96		100.5018

				80.98		100.5078

				81		100.5078

				81.02		100.5078

				81.04		100.5078

				81.07		100.5018

				81.09		100.5018

				81.11		100.5018

				81.13		100.5018

				81.15		100.5018

				81.17		100.5018

				81.19		100.5018

				81.21		100.5018

				81.23		100.5018

				81.26		100.5018

				81.28		100.5018

				81.3		100.5018

				81.32		100.5078

				81.34		100.5078

				81.36		100.5078

				81.38		100.5078

				81.4		100.5078

				81.42		100.5078

				81.45		100.5078

				81.47		100.5078

				81.49		100.5078

				81.51		100.5078

				81.53		100.5078

				81.55		100.5078

				81.57		100.5078

				81.59		100.5078

				81.61		100.5078

				81.63		100.5078

				81.66		100.5018

				81.68		100.5078

				81.7		100.5018

				81.72		100.5018

				81.74		100.5018

				81.76		100.5018

				81.78		100.5018

				81.8		100.5078

				81.82		100.5018

				81.85		100.5078

				81.87		100.5078

				81.89		100.5078

				81.91		100.5078

				81.93		100.5018

				81.95		100.5018

				81.97		100.5018

				81.99		100.5078

				82.01		100.5018

				82.04		100.5018

				82.06		100.5018

				82.08		100.5018

				82.1		100.5018

				82.12		100.5018

				82.14		100.5018

				82.16		100.5018

				82.18		100.5018

				82.2		100.5018

				82.22		100.5018

				82.25		100.5018

				82.27		100.5018

				82.29		100.5078

				82.31		100.5078

				82.33		100.5078

				82.35		100.5078

				82.37		100.5018

				82.39		100.5018

				82.41		100.5018

				82.44		100.5078

				82.46		100.5018

				82.48		100.5018

				82.5		100.5018

				82.52		100.5018

				82.54		100.5018

				82.56		100.5018

				82.58		100.5018

				82.6		100.5018

				82.63		100.5018

				82.65		100.5018

				82.67		100.5018

				82.69		100.5078

				82.71		100.5018

				82.73		100.5018

				82.75		100.5018

				82.77		100.5018

				82.79		100.5018

				82.81		100.5018

				82.84		100.5018

				82.86		100.5018

				82.88		100.5018

				82.9		100.5018

				82.92		100.5018

				82.94		100.5018

				82.96		100.5018

				82.98		100.5018

				83		100.5018

				83.03		100.5018

				83.05		100.5018

				83.07		100.5018

				83.09		100.5018

				83.11		100.5018

				83.13		100.5018

				83.15		100.5018

				83.17		100.5018

				83.19		100.5018

				83.22		100.5018

				83.24		100.5018

				83.26		100.5018

				83.28		100.5018

				83.3		100.5018

				83.32		100.5018

				83.34		100.5018

				83.36		100.5078

				83.38		100.5018

				83.41		100.5018

				83.43		100.5018

				83.45		100.5018

				83.47		100.5018

				83.49		100.5018

				83.51		100.5018

				83.53		100.5018

				83.55		100.5018

				83.57		100.5018

				83.59		100.5018

				83.62		100.5018

				83.64		100.5018

				83.66		100.5018

				83.68		100.5018

				83.7		100.5018

				83.72		100.5018

				83.74		100.5018

				83.76		100.5018

				83.78		100.5018

				83.81		100.5018

				83.83		100.5018

				83.85		100.5018

				83.87		100.5018

				83.89		100.5018

				83.91		100.5018

				83.93		100.5018

				83.95		100.5018

				83.97		100.5018

				84		100.5018

				84.02		100.5018

				84.04		100.5018

				84.06		100.5018

				84.08		100.5018

				84.1		100.4958

				84.12		100.4958

				84.14		100.4958

				84.16		100.4958

				84.19		100.4958

				84.21		100.4958

				84.23		100.4958

				84.25		100.4958

				84.27		100.4958

				84.29		100.4958

				84.31		100.4958

				84.33		100.4958

				84.35		100.4958

				84.37		100.4958

				84.4		100.4958

				84.42		100.4958

				84.44		100.4958

				84.46		100.4958

				84.48		100.4958

				84.5		100.4958

				84.52		100.4958

				84.54		100.4958

				84.56		100.4958

				84.59		100.4958

				84.61		100.4958

				84.63		100.4958

				84.65		100.4958

				84.67		100.4958

				84.69		100.4958

				84.71		100.4958

				84.73		100.4958

				84.75		100.4958

				84.78		100.4958

				84.8		100.4958

				84.82		100.4958

				84.84		100.4958

				84.86		100.5018

				84.88		100.5018

				84.9		100.4958

				84.92		100.4958

				84.94		100.4958

				84.97		100.4958

				84.99		100.4958

				85.01		100.4958

				85.03		100.4958

				85.05		100.4958

				85.07		100.4898

				85.09		100.4958

				85.11		100.4958

				85.13		100.4958

				85.16		100.4958

				85.18		100.4958

				85.2		100.4898

				85.22		100.4958

				85.24		100.4898

				85.26		100.4898

				85.28		100.4898

				85.3		100.4898

				85.32		100.4898

				85.35		100.4898

				85.37		100.4898

				85.39		100.4898

				85.41		100.4958

				85.43		100.4898

				85.45		100.4898

				85.47		100.4958

				85.49		100.4898

				85.51		100.4898

				85.54		100.4898

				85.56		100.4898

				85.58		100.4898

				85.6		100.4898

				85.62		100.4958

				85.64		100.4898

				85.66		100.4898

				85.68		100.4898

				85.7		100.4898

				85.72		100.4958

				85.75		100.4898

				85.77		100.4898

				85.79		100.4958

				85.81		100.4958

				85.83		100.4958

				85.85		100.4958

				85.87		100.4958

				85.89		100.4958

				85.91		100.4958

				85.94		100.4958

				85.96		100.4958

				85.98		100.4958

				86		100.4958

				86.02		100.4958

				86.04		100.4958

				86.06		100.4958

				86.08		100.4958

				86.1		100.4958

				86.13		100.4958

				86.15		100.4958

				86.17		100.4958

				86.19		100.4958

				86.21		100.4958

				86.23		100.4958

				86.25		100.4958

				86.27		100.4958

				86.29		100.4958

				86.32		100.4958

				86.34		100.4958

				86.36		100.4958

				86.38		100.4958

				86.4		100.4958

				86.42		100.4958

				86.44		100.4958

				86.46		100.5018

				86.48		100.4958

				86.51		100.5018

				86.53		100.5018

				86.55		100.5018

				86.57		100.5018

				86.59		100.5018

				86.61		100.5018

				86.63		100.5018

				86.65		100.5018

				86.67		100.5018

				86.7		100.5018

				86.72		100.5018

				86.74		100.5018

				86.76		100.5018

				86.78		100.5018

				86.8		100.5018

				86.82		100.4958

				86.84		100.5018

				86.86		100.5018

				86.88		100.5018

				86.91		100.5018

				86.93		100.5018

				86.95		100.4958

				86.97		100.5018

				86.99		100.5018

				87.01		100.5018

				87.03		100.5018

				87.05		100.5018

				87.07		100.5018

				87.1		100.5018

				87.12		100.5018

				87.14		100.5078

				87.16		100.5078

				87.18		100.5018

				87.2		100.5078

				87.22		100.5078

				87.24		100.5078

				87.26		100.5078

				87.29		100.5078

				87.31		100.5078

				87.33		100.5078

				87.35		100.5078

				87.37		100.5078

				87.39		100.5078

				87.41		100.5078

				87.43		100.5078

				87.45		100.5137

				87.48		100.5078

				87.5		100.5078

				87.52		100.5078

				87.54		100.5078

				87.56		100.5078

				87.58		100.5078

				87.6		100.5078

				87.62		100.5078

				87.64		100.5078

				87.67		100.5078

				87.69		100.5078

				87.71		100.5078

				87.73		100.5078

				87.75		100.5078

				87.77		100.5078

				87.79		100.5137

				87.81		100.5137

				87.83		100.5137

				87.85		100.5137

				87.88		100.5137

				87.9		100.5137

				87.92		100.5137

				87.94		100.5137

				87.96		100.5137

				87.98		100.5137

				88		100.5137

				88.02		100.5137

				88.04		100.5137

				88.07		100.5137

				88.09		100.5137

				88.11		100.5137

				88.13		100.5137

				88.15		100.5137

				88.17		100.5137

				88.19		100.5137

				88.21		100.5137

				88.23		100.5137

				88.26		100.5137

				88.28		100.5137

				88.3		100.5137

				88.32		100.5137

				88.34		100.5137

				88.36		100.5137

				88.38		100.5137

				88.4		100.5137

				88.42		100.5137

				88.45		100.5137

				88.47		100.5137

				88.49		100.5137

				88.51		100.5137

				88.53		100.5137

				88.55		100.5137

				88.57		100.5137

				88.59		100.5137

				88.61		100.5137

				88.63		100.5137

				88.66		100.5137

				88.68		100.5137

				88.7		100.5137

				88.72		100.5137

				88.74		100.5137

				88.76		100.5137

				88.78		100.5137

				88.8		100.5137

				88.82		100.5137

				88.85		100.5137

				88.87		100.5137

				88.89		100.5137

				88.91		100.5137

				88.93		100.5137

				88.95		100.5137

				88.97		100.5137

				88.99		100.5078

				89.01		100.5078

				89.04		100.5137

				89.06		100.5078

				89.08		100.5078

				89.1		100.5078

				89.12		100.5078

				89.14		100.5078

				89.16		100.5078

				89.18		100.5078

				89.2		100.5078

				89.22		100.5078

				89.25		100.5078

				89.27		100.5078

				89.29		100.5078

				89.31		100.5078

				89.33		100.5078

				89.35		100.5078

				89.37		100.5078

				89.39		100.5078

				89.41		100.5078

				89.44		100.5078

				89.46		100.5078

				89.48		100.5078

				89.5		100.5078

				89.52		100.5078

				89.54		100.5078

				89.56		100.5078

				89.58		100.5078

				89.6		100.5078

				89.63		100.5078

				89.65		100.5137

				89.67		100.5137

				89.69		100.5137

				89.71		100.5137

				89.73		100.5137

				89.75		100.5137

				89.77		100.5137

				89.79		100.5137

				89.81		100.5137

				89.84		100.5137

				89.86		100.5137

				89.88		100.5137

				89.9		100.5137

				89.92		100.5137

				89.94		100.5137

				89.96		100.5137

				89.98		100.5137

				90		100.5137

				90.03		100.5137

				90.05		100.5137

				90.07		100.5137

				90.09		100.5137

				90.11		100.5137

				90.13		100.5137

				90.15		100.5078

				90.17		100.5078

				90.19		100.5137

				90.21		100.5078

				90.24		100.5137

				90.26		100.5137

				90.28		100.5137

				90.3		100.5137

				90.32		100.5137

				90.34		100.5137

				90.36		100.5137

				90.38		100.5137

				90.4		100.5137

				90.43		100.5137

				90.45		100.5137

				90.47		100.5137

				90.49		100.5137

				90.51		100.5137

				90.53		100.5137

				90.55		100.5137

				90.57		100.5137

				90.59		100.5137

				90.62		100.5137

				90.64		100.5137

				90.66		100.5137

				90.68		100.5137

				90.7		100.5137

				90.72		100.5137

				90.74		100.5137

				90.76		100.5137

				90.78		100.5137

				90.8		100.5137

				90.83		100.5137

				90.85		100.5197

				90.87		100.5197

				90.89		100.5197

				90.91		100.5197

				90.93		100.5197

				90.95		100.5137

				90.97		100.5197

				90.99		100.5197

				91.02		100.5197

				91.04		100.5197

				91.06		100.5197

				91.08		100.5197

				91.1		100.5197

				91.12		100.5197

				91.14		100.5197

				91.16		100.5197

				91.18		100.5197

				91.21		100.5197

				91.23		100.5197

				91.25		100.5197

				91.27		100.5197

				91.29		100.5197

				91.31		100.5197

				91.33		100.5197

				91.35		100.5197

				91.37		100.5197

				91.39		100.5197

				91.42		100.5197

				91.44		100.5197

				91.46		100.5197

				91.48		100.5197

				91.5		100.5197

				91.52		100.5197

				91.54		100.5197

				91.56		100.5197

				91.58		100.5197

				91.61		100.5197

				91.63		100.5197

				91.65		100.5197

				91.67		100.5197

				91.69		100.5197

				91.71		100.5197

				91.73		100.5197

				91.75		100.5197

				91.77		100.5197

				91.79		100.5197

				91.82		100.5197

				91.84		100.5197

				91.86		100.5197

				91.88		100.5197

				91.9		100.5197

				91.92		100.5197

				91.94		100.5197

				91.96		100.5197

				91.98		100.5197

				92.01		100.5197

				92.03		100.5197

				92.05		100.5197

				92.07		100.5197

				92.09		100.5197

				92.11		100.5197

				92.13		100.5197

				92.15		100.5197

				92.17		100.5197

				92.2		100.5197

				92.22		100.5197

				92.24		100.5197

				92.26		100.5197

				92.28		100.5197

				92.3		100.5197

				92.32		100.5197

				92.34		100.5197

				92.36		100.5197

				92.38		100.5197

				92.41		100.5197

				92.43		100.5197

				92.45		100.5197

				92.47		100.5197

				92.49		100.5197

				92.51		100.5197

				92.53		100.5197

				92.55		100.5197

				92.57		100.5197

				92.6		100.5197

				92.62		100.5197

				92.64		100.5197

				92.66		100.5197

				92.68		100.5197

				92.7		100.5197

				92.72		100.5197

				92.74		100.5197

				92.76		100.5197

				92.78		100.5197

				92.81		100.5197

				92.83		100.5197

				92.85		100.5197

				92.87		100.5197

				92.89		100.5197

				92.91		100.5197

				92.93		100.5197

				92.95		100.5197

				92.97		100.5197

				93		100.5257

				93.02		100.5257

				93.04		100.5257

				93.06		100.5257

				93.08		100.5257

				93.1		100.5257

				93.12		100.5257

				93.14		100.5257

				93.16		100.5257

				93.18		100.5257

				93.21		100.5257

				93.23		100.5257

				93.25		100.5257

				93.27		100.5257

				93.29		100.5257

				93.31		100.5257

				93.33		100.5257

				93.35		100.5257

				93.37		100.5257

				93.4		100.5257

				93.42		100.5257

				93.44		100.5257

				93.46		100.5257

				93.48		100.5317

				93.5		100.5317

				93.52		100.5257

				93.54		100.5257

				93.56		100.5317

				93.59		100.5317

				93.61		100.5257

				93.63		100.5317

				93.65		100.5317

				93.67		100.5317

				93.69		100.5317

				93.71		100.5317

				93.73		100.5257

				93.75		100.5317

				93.77		100.5317

				93.8		100.5317

				93.82		100.5317

				93.84		100.5317

				93.86		100.5257

				93.88		100.5257

				93.9		100.5257

				93.92		100.5257

				93.94		100.5257

				93.96		100.5257

				93.99		100.5257

				94.01		100.5257

				94.03		100.5257

				94.05		100.5257

				94.07		100.5257

				94.09		100.5257

				94.11		100.5257

				94.13		100.5257

				94.15		100.5257

				94.17		100.5257

				94.2		100.5257

				94.22		100.5257

				94.24		100.5257

				94.26		100.5257

				94.28		100.5257

				94.3		100.5257

				94.32		100.5257

				94.34		100.5257

				94.36		100.5257

				94.39		100.5257

				94.41		100.5257

				94.43		100.5257

				94.45		100.5257

				94.47		100.5257

				94.49		100.5257

				94.51		100.5257

				94.53		100.5257

				94.55		100.5257

				94.58		100.5257

				94.6		100.5257

				94.62		100.5257

				94.64		100.5257

				94.66		100.5257

				94.68		100.5257

				94.7		100.5257

				94.72		100.5257

				94.74		100.5197

				94.76		100.5257

				94.79		100.5257

				94.81		100.5197

				94.83		100.5197

				94.85		100.5197

				94.87		100.5197

				94.89		100.5197

				94.91		100.5197

				94.93		100.5197

				94.95		100.5197

				94.98		100.5197

				95		100.5197

				95.02		100.5197

				95.04		100.5197

				95.06		100.5197

				95.08		100.5197

				95.1		100.5197

				95.12		100.5197

				95.14		100.5197

				95.16		100.5197

				95.19		100.5197

				95.21		100.5197

				95.23		100.5197

				95.25		100.5197

				95.27		100.5197

				95.29		100.5197

				95.31		100.5197

				95.33		100.5197

				95.35		100.5197

				95.38		100.5197

				95.4		100.5197

				95.42		100.5197

				95.44		100.5197

				95.46		100.5137

				95.48		100.5137

				95.5		100.5137

				95.52		100.5137

				95.54		100.5137

				95.56		100.5137

				95.59		100.5137

				95.61		100.5137

				95.63		100.5137

				95.65		100.5137

				95.67		100.5137

				95.69		100.5137

				95.71		100.5137

				95.73		100.5137

				95.75		100.5197

				95.78		100.5197

				95.8		100.5137

				95.82		100.5137

				95.84		100.5137

				95.86		100.5137

				95.88		100.5137

				95.9		100.5137

				95.92		100.5197

				95.94		100.5137

				95.96		100.5137

				95.99		100.5137

				96.01		100.5137

				96.03		100.5137

				96.05		100.5197

				96.07		100.5197

				96.09		100.5137

				96.11		100.5197

				96.13		100.5197

				96.15		100.5197

				96.18		100.5197

				96.2		100.5197

				96.22		100.5197

				96.24		100.5197

				96.26		100.5197

				96.28		100.5197

				96.3		100.5197

				96.32		100.5197

				96.34		100.5197

				96.36		100.5197

				96.39		100.5197

				96.41		100.5197

				96.43		100.5197

				96.45		100.5197

				96.47		100.5197

				96.49		100.5197

				96.51		100.5197

				96.53		100.5197

				96.55		100.5197

				96.58		100.5197

				96.6		100.5197

				96.62		100.5197

				96.64		100.5197

				96.66		100.5197

				96.68		100.5197

				96.7		100.5197

				96.72		100.5197

				96.74		100.5197

				96.77		100.5197

				96.79		100.5197

				96.81		100.5197

				96.83		100.5197

				96.85		100.5197

				96.87		100.5197

				96.89		100.5197

				96.91		100.5197

				96.93		100.5197

				96.95		100.5197

				96.98		100.5197

				97		100.5197

				97.02		100.5197

				97.04		100.5197

				97.06		100.5197

				97.08		100.5197

				97.1		100.5197

				97.12		100.5197

				97.14		100.5197

				97.17		100.5197

				97.19		100.5197

				97.21		100.5197

				97.23		100.5197

				97.25		100.5197

				97.27		100.5197

				97.29		100.5197

				97.31		100.5197

				97.33		100.5197

				97.35		100.5197

				97.38		100.5197

				97.4		100.5197

				97.42		100.5197

				97.44		100.5197

				97.46		100.5197

				97.48		100.5197

				97.5		100.5197

				97.52		100.5197

				97.54		100.5197

				97.56		100.5197

				97.59		100.5257

				97.61		100.5257

				97.63		100.5257

				97.65		100.5257

				97.67		100.5257

				97.69		100.5257

				97.71		100.5257

				97.73		100.5257

				97.75		100.5257

				97.78		100.5257

				97.8		100.5257

				97.82		100.5257

				97.84		100.5257

				97.86		100.5257

				97.88		100.5257

				97.9		100.5257

				97.92		100.5257

				97.94		100.5257

				97.96		100.5257

				97.99		100.5257

				98.01		100.5257

				98.03		100.5257

				98.05		100.5257

				98.07		100.5257

				98.09		100.5257

				98.11		100.5257

				98.13		100.5257

				98.15		100.5257

				98.18		100.5257

				98.2		100.5257

				98.22		100.5257

				98.24		100.5317

				98.26		100.5317

				98.28		100.5317

				98.3		100.5317

				98.32		100.5317

				98.34		100.5317

				98.36		100.5317

				98.39		100.5317

				98.41		100.5317

				98.43		100.5317

				98.45		100.5317

				98.47		100.5317

				98.49		100.5317

				98.51		100.5317

				98.53		100.5317

				98.55		100.5317

				98.58		100.5317

				98.6		100.5317

				98.62		100.5317

				98.64		100.5317

				98.66		100.5317

				98.68		100.5317

				98.7		100.5317

				98.72		100.5317

				98.74		100.5317

				98.77		100.5376

				98.79		100.5376

				98.81		100.5376

				98.83		100.5376

				98.85		100.5376

				98.87		100.5376

				98.89		100.5376

				98.91		100.5376

				98.93		100.5376

				98.95		100.5376

				98.98		100.5376

				99		100.5376

				99.02		100.5376

				99.04		100.5376

				99.06		100.5376

				99.08		100.5376

				99.1		100.5376

				99.12		100.5376

				99.14		100.5376

				99.17		100.5376

				99.19		100.5436

				99.21		100.5436

				99.23		100.5436

				99.25		100.5436

				99.27		100.5436

				99.29		100.5436

				99.31		100.5436

				99.33		100.5436

				99.35		100.5436

				99.38		100.5436

				99.4		100.5436

				99.42		100.5436

				99.44		100.5436

				99.46		100.5436

				99.48		100.5436

				99.5		100.5436

				99.52		100.5436

				99.54		100.5436

				99.57		100.5436

				99.59		100.5376

				99.61		100.5376

				99.63		100.5436

				99.65		100.5376

				99.67		100.5376

				99.69		100.5376

				99.71		100.5436

				99.73		100.5376

				99.75		100.5436

				99.78		100.5436

				99.8		100.5436

				99.82		100.5436

				99.84		100.5436

				99.86		100.5436

				99.88		100.5436

				99.9		100.5436

				99.92		100.5436

				99.94		100.5436

				99.97		100.5436

				99.99		100.5436

				100.01		100.5436

				100.03		100.5436

				100.05		100.5436

				100.07		100.5436

				100.09		100.5436

				100.11		100.5436

				100.13		100.5436

				100.15		100.5436

				100.18		100.5436

				100.2		100.5436

				100.22		100.5436

				100.24		100.5436

				100.26		100.5436

				100.28		100.5436

				100.3		100.5436

				100.32		100.5436

				100.34		100.5436

				100.36		100.5436

				100.39		100.5436

				100.41		100.5436

				100.43		100.5436

				100.45		100.5436

				100.47		100.5436

				100.49		100.5436

				100.51		100.5436

				100.53		100.5436

				100.55		100.5436

				100.57		100.5436

				100.6		100.5436

				100.62		100.5436

				100.64		100.5436

				100.66		100.5376

				100.68		100.5436

				100.7		100.5436

				100.72		100.5436

				100.74		100.5376

				100.76		100.5376

				100.79		100.5376

				100.81		100.5376

				100.83		100.5376

				100.85		100.5376

				100.87		100.5376

				100.89		100.5376

				100.91		100.5376

				100.93		100.5376

				100.95		100.5376

				100.97		100.5376

				101		100.5376

				101.02		100.5376

				101.04		100.5376

				101.06		100.5376

				101.08		100.5317

				101.1		100.5317

				101.12		100.5317

				101.14		100.5317

				101.16		100.5317

				101.19		100.5317

				101.21		100.5317

				101.23		100.5317

				101.25		100.5317

				101.27		100.5317

				101.29		100.5317

				101.31		100.5317

				101.33		100.5317

				101.35		100.5317

				101.37		100.5317

				101.4		100.5317

				101.42		100.5317

				101.44		100.5317

				101.46		100.5317

				101.48		100.5317

				101.5		100.5317

				101.52		100.5317

				101.54		100.5317

				101.56		100.5317

				101.59		100.5317

				101.61		100.5317

				101.63		100.5317

				101.65		100.5317

				101.67		100.5317

				101.69		100.5317

				101.71		100.5317

				101.73		100.5317

				101.75		100.5317

				101.77		100.5317

				101.8		100.5257

				101.82		100.5257

				101.84		100.5257

				101.86		100.5257

				101.88		100.5257

				101.9		100.5257

				101.92		100.5257

				101.94		100.5257

				101.96		100.5257

				101.99		100.5257

				102.01		100.5257

				102.03		100.5257

				102.05		100.5257

				102.07		100.5257

				102.09		100.5257

				102.11		100.5257

				102.13		100.5197

				102.15		100.5197

				102.17		100.5197

				102.2		100.5197

				102.22		100.5197

				102.24		100.5257

				102.26		100.5257

				102.28		100.5197

				102.3		100.5197

				102.32		100.5197

				102.34		100.5197

				102.36		100.5197

				102.39		100.5197

				102.41		100.5197

				102.43		100.5197

				102.45		100.5197

				102.47		100.5197

				102.49		100.5197

				102.51		100.5197

				102.53		100.5197

				102.55		100.5197

				102.57		100.5197

				102.6		100.5197

				102.62		100.5197

				102.64		100.5197

				102.66		100.5197

				102.68		100.5197

				102.7		100.5197

				102.72		100.5197

				102.74		100.5197

				102.76		100.5197

				102.78		100.5197

				102.81		100.5197

				102.83		100.5197

				102.85		100.5197

				102.87		100.5197

				102.89		100.5197

				102.91		100.5197

				102.93		100.5197

				102.95		100.5197

				102.97		100.5197

				103		100.5197

				103.02		100.5197

				103.04		100.5197

				103.06		100.5197

				103.08		100.5197

				103.1		100.5197

				103.12		100.5197

				103.14		100.5197

				103.16		100.5197

				103.18		100.5197

				103.21		100.5197

				103.23		100.5197

				103.25		100.5197

				103.27		100.5197

				103.29		100.5137

				103.31		100.5137

				103.33		100.5197

				103.35		100.5137

				103.37		100.5137

				103.39		100.5137

				103.42		100.5137

				103.44		100.5137

				103.46		100.5137

				103.48		100.5137

				103.5		100.5137

				103.52		100.5137

				103.54		100.5137

				103.56		100.5137

				103.58		100.5137

				103.61		100.5137

				103.63		100.5137

				103.65		100.5137

				103.67		100.5137

				103.69		100.5137

				103.71		100.5137

				103.73		100.5137

				103.75		100.5137

				103.77		100.5137

				103.79		100.5137

				103.82		100.5137

				103.84		100.5137

				103.86		100.5137

				103.88		100.5137

				103.9		100.5137

				103.92		100.5137

				103.94		100.5137

				103.96		100.5137

				103.98		100.5137

				104.01		100.5137

				104.03		100.5137

				104.05		100.5078

				104.07		100.5078

				104.09		100.5078

				104.11		100.5078

				104.13		100.5078

				104.15		100.5078

				104.17		100.5078

				104.19		100.5137

				104.22		100.5137

				104.24		100.5137

				104.26		100.5137

				104.28		100.5078

				104.3		100.5137

				104.32		100.5078

				104.34		100.5078

				104.36		100.5078

				104.38		100.5078

				104.4		100.5078

				104.43		100.5078

				104.45		100.5078

				104.47		100.5078

				104.49		100.5078

				104.51		100.5078

				104.53		100.5078

				104.55		100.5078

				104.57		100.5078

				104.59		100.5078

				104.62		100.5078

				104.64		100.5078

				104.66		100.5078

				104.68		100.5078

				104.7		100.5078

				104.72		100.5078

				104.74		100.5078

				104.76		100.5078

				104.78		100.5078

				104.8		100.5078

				104.83		100.5078

				104.85		100.5078

				104.87		100.5078

				104.89		100.5078

				104.91		100.5078

				104.93		100.5078

				104.95		100.5078

				104.97		100.5078

				104.99		100.5078

				105.02		100.5078

				105.04		100.5078

				105.06		100.5078

				105.08		100.5078

				105.1		100.5078

				105.12		100.5078

				105.14		100.5078

				105.16		100.5078

				105.18		100.5078

				105.2		100.5078

				105.23		100.5078

				105.25		100.5078

				105.27		100.5078

				105.29		100.5078

				105.31		100.5078

				105.33		100.5078

				105.35		100.5078

				105.37		100.5078

				105.39		100.5078

				105.42		100.5078

				105.44		100.5078

				105.46		100.5078

				105.48		100.5078

				105.5		100.5078

				105.52		100.5078

				105.54		100.5078

				105.56		100.5078

				105.58		100.5137

				105.6		100.5137

				105.63		100.5137

				105.65		100.5137

				105.67		100.5137

				105.69		100.5137

				105.71		100.5137

				105.73		100.5137

				105.75		100.5137

				105.77		100.5137

				105.79		100.5137

				105.81		100.5137

				105.84		100.5137

				105.86		100.5137

				105.88		100.5137

				105.9		100.5137

				105.92		100.5137

				105.94		100.5137

				105.96		100.5137

				105.98		100.5137

				106		100.5137

				106.03		100.5137

				106.05		100.5137

				106.07		100.5137

				106.09		100.5137

				106.11		100.5137

				106.13		100.5137

				106.15		100.5137

				106.17		100.5137

				106.19		100.5137

				106.21		100.5137

				106.24		100.5137

				106.26		100.5137

				106.28		100.5137

				106.3		100.5137

				106.32		100.5137

				106.34		100.5137

				106.36		100.5137

				106.38		100.5137

				106.4		100.5137

				106.42		100.5137

				106.45		100.5137

				106.47		100.5137

				106.49		100.5137

				106.51		100.5137

				106.53		100.5137

				106.55		100.5137

				106.57		100.5137

				106.59		100.5137

				106.61		100.5137

				106.64		100.5137

				106.66		100.5137

				106.68		100.5137

				106.7		100.5137

				106.72		100.5137

				106.74		100.5137

				106.76		100.5137

				106.78		100.5078

				106.8		100.5078

				106.82		100.5078

				106.85		100.5137

				106.87		100.5078

				106.89		100.5078

				106.91		100.5078

				106.93		100.5078

				106.95		100.5078

				106.97		100.5078

				106.99		100.5078

				107.01		100.5078

				107.04		100.5078

				107.06		100.5078

				107.08		100.5078

				107.1		100.5078

				107.12		100.5078

				107.14		100.5078

				107.16		100.5078

				107.18		100.5137

				107.2		100.5137

				107.22		100.5078

				107.25		100.5078

				107.27		100.5137

				107.29		100.5078

				107.31		100.5137

				107.33		100.5078

				107.35		100.5078

				107.37		100.5078

				107.39		100.5078

				107.41		100.5078

				107.44		100.5078

				107.46		100.5078

				107.48		100.5078

				107.5		100.5078

				107.52		100.5078

				107.54		100.5078

				107.56		100.5078

				107.58		100.5078

				107.6		100.5078

				107.62		100.5078

				107.65		100.5078

				107.67		100.5078

				107.69		100.5078

				107.71		100.5078

				107.73		100.5078

				107.75		100.5078

				107.77		100.5078

				107.79		100.5078

				107.81		100.5078

				107.83		100.5078

				107.86		100.5078

				107.88		100.5078

				107.9		100.5078

				107.92		100.5078

				107.94		100.5078

				107.96		100.5078

				107.98		100.5078

				108		100.5018

				108.02		100.5078

				108.05		100.5078

				108.07		100.5018

				108.09		100.5078

				108.11		100.5078

				108.13		100.5078

				108.15		100.5078

				108.17		100.5078

				108.19		100.5078

				108.21		100.5078

				108.23		100.5078

				108.26		100.5078

				108.28		100.5078

				108.3		100.5078

				108.32		100.5078

				108.34		100.5078

				108.36		100.5078

				108.38		100.5078

				108.4		100.5078

				108.42		100.5078

				108.44		100.5078

				108.47		100.5078

				108.49		100.5078

				108.51		100.5078

				108.53		100.5078

				108.55		100.5078

				108.57		100.5078

				108.59		100.5078

				108.61		100.5078

				108.63		100.5078

				108.66		100.5078

				108.68		100.5078

				108.7		100.5078

				108.72		100.5078

				108.74		100.5078

				108.76		100.5078

				108.78		100.5078

				108.8		100.5078

				108.82		100.5078

				108.84		100.5078

				108.87		100.5078

				108.89		100.5078

				108.91		100.5078

				108.93		100.5078

				108.95		100.5078

				108.97		100.5078

				108.99		100.5078

				109.01		100.5078

				109.03		100.5078

				109.05		100.5078

				109.08		100.5078

				109.1		100.5078

				109.12		100.5078

				109.14		100.5078

				109.16		100.5078

				109.18		100.5078

				109.2		100.5078

				109.22		100.5078

				109.24		100.5078

				109.26		100.5078

				109.29		100.5078

				109.31		100.5078

				109.33		100.5078

				109.35		100.5078

				109.37		100.5078

				109.39		100.5078

				109.41		100.5078

				109.43		100.5078

				109.45		100.5078

				109.47		100.5078

				109.5		100.5078

				109.52		100.5078

				109.54		100.5078

				109.56		100.5078

				109.58		100.5078

				109.6		100.5078

				109.62		100.5137

				109.64		100.5078

				109.66		100.5078

				109.69		100.5078

				109.71		100.5137

				109.73		100.5137

				109.75		100.5137

				109.77		100.5137

				109.79		100.5137

				109.81		100.5078

				109.83		100.5078

				109.85		100.5078

				109.87		100.5137

				109.9		100.5078

				109.92		100.5137

				109.94		100.5137

				109.96		100.5137

				109.98		100.5018

				110		100.5018

				110.02		100.5018

				110.04		100.5018

				110.06		100.5018

				110.08		100.5018

				110.11		100.5018

				110.13		100.5018

				110.15		100.5018

				110.17		100.5018

				110.19		100.4779

				110.21		100.4779

				110.23		100.4779

				110.25		100.4779

				110.27		100.4779

				110.29		100.4719

				110.32		100.4719

				110.34		100.4719

				110.36		100.4719

				110.38		100.4719

				110.4		100.4719

				110.42		100.4779

				110.44		100.4779

				110.46		100.4779

				110.48		100.4839

				110.51		100.4839

				110.53		100.4839

				110.55		100.4898

				110.57		100.4958

				110.59		100.5018

				110.61		100.5078

				110.63		100.5137

				110.65		100.5137

				110.67		100.5137

				110.69		100.5197

				110.72		100.5197

				110.74		100.5197

				110.76		100.5197

				110.78		100.5197

				110.8		100.5197

				110.82		100.5257

				110.84		100.5197

				110.86		100.5257

				110.88		100.5257

				110.9		100.5257

				110.93		100.5197

				110.95		100.5257

				110.97		100.5257

				110.99		100.5197

				111.01		100.5197

				111.03		100.5257

				111.05		100.5257

				111.07		100.5257

				111.09		100.5257

				111.11		100.5257

				111.14		100.5257

				111.16		100.5257

				111.18		100.5257

				111.2		100.5257

				111.22		100.5257

				111.24		100.5257

				111.26		100.5257

				111.28		100.5257

				111.3		100.5257

				111.32		100.5257

				111.35		100.5257

				111.37		100.5257

				111.39		100.5257

				111.41		100.5257

				111.43		100.5257

				111.45		100.5317

				111.47		100.5317

				111.49		100.5317

				111.51		100.5257

				111.53		100.5496

				111.56		100.5436

				111.58		100.5436

				111.6		100.5436

				111.62		100.5436

				111.64		100.5376

				111.66		100.5376

				111.68		100.5376

				111.7		100.5376

				111.72		100.5376

				111.75		100.5376

				111.77		100.5376

				111.79		100.5317

				111.81		100.5317

				111.83		100.5317

				111.85		100.5317

				111.87		100.5317

				111.89		100.5317

				111.91		100.5317

				111.93		100.5317

				111.96		100.5317

				111.98		100.5317

				112		100.5317

				112.02		100.5317

				112.04		100.5257

				112.06		100.5257

				112.08		100.5436

				112.1		100.5496

				112.12		100.5496

				112.14		100.5496

				112.17		100.5496

				112.19		100.5496

				112.21		100.5496

				112.23		100.5496

				112.25		100.5496

				112.27		100.5496

				112.29		100.5496

				112.31		100.5436

				112.33		100.5376

				112.36		100.5317

				112.38		100.5257

				112.4		100.5197

				112.42		100.5137

				112.44		100.5137

				112.46		100.5078

				112.48		100.5078

				112.5		100.5078

				112.52		100.5078

				112.54		100.5078

				112.57		100.5078

				112.59		100.5078

				112.61		100.5078

				112.63		100.5078

				112.65		100.5078

				112.67		100.5078

				112.69		100.5078

				112.71		100.5078

				112.73		100.5078

				112.75		100.5078

				112.78		100.5078

				112.8		100.5078

				112.82		100.5078

				112.84		100.5078

				112.86		100.5078

				112.88		100.5078

				112.9		100.5078

				112.92		100.5078

				112.94		100.5078

				112.96		100.5078

				112.99		100.5078

				113.01		100.5137

				113.03		100.5078

				113.05		100.5078

				113.07		100.5078

				113.09		100.5078

				113.11		100.5078

				113.13		100.5078

				113.15		100.5078

				113.18		100.5137

				113.2		100.5137

				113.22		100.5137

				113.24		100.5137

				113.26		100.5137

				113.28		100.5137

				113.3		100.5137

				113.32		100.5137

				113.34		100.5137

				113.36		100.5137

				113.39		100.5137

				113.41		100.5137

				113.43		100.5137

				113.45		100.5137

				113.47		100.5137

				113.49		100.5137

				113.51		100.5137

				113.53		100.5137

				113.55		100.5078

				113.57		100.5137

				113.6		100.5137

				113.62		100.5137

				113.64		100.5137

				113.66		100.5137

				113.68		100.5137

				113.7		100.5137

				113.72		100.5137

				113.74		100.5137

				113.76		100.5137

				113.78		100.5137

				113.81		100.5137

				113.83		100.5137

				113.85		100.5137

				113.87		100.5137

				113.89		100.5137

				113.91		100.5137

				113.93		100.5137

				113.95		100.5137

				113.97		100.5137

				113.99		100.5137

				114.02		100.5137

				114.04		100.5137

				114.06		100.5137

				114.08		100.5137

				114.1		100.5137

				114.12		100.5137

				114.14		100.5137

				114.16		100.5137

				114.18		100.5137

				114.2		100.5137

				114.23		100.5137

				114.25		100.5137

				114.27		100.5137

				114.29		100.5137

				114.31		100.5137

				114.33		100.5078

				114.35		100.5137

				114.37		100.5137

				114.39		100.5137

				114.41		100.5078

				114.44		100.5137

				114.46		100.5078

				114.48		100.5078

				114.5		100.5078

				114.52		100.5078

				114.54		100.5078

				114.56		100.5078

				114.58		100.5078

				114.6		100.5078

				114.63		100.5078

				114.65		100.5078

				114.67		100.5078

				114.69		100.5078

				114.71		100.5078

				114.73		100.5078

				114.75		100.5078

				114.77		100.5078

				114.79		100.5137

				114.81		100.5078

				114.84		100.5078

				114.86		100.5078

				114.88		100.5078

				114.9		100.5078

				114.92		100.5078

				114.94		100.5078

				114.96		100.5078

				114.98		100.5078

				115		100.5078

				115.02		100.5078

				115.05		100.5078

				115.07		100.5078

				115.09		100.5078

				115.11		100.5078

				115.13		100.5078

				115.15		100.5078

				115.17		100.5078

				115.19		100.5078

				115.21		100.5078

				115.23		100.5078

				115.26		100.5078

				115.28		100.5078

				115.3		100.5078

				115.32		100.5078

				115.34		100.5078

				115.36		100.5078

				115.38		100.5078

				115.4		100.5018

				115.42		100.5078

				115.44		100.5078

				115.47		100.5078

				115.49		100.5078

				115.51		100.5018

				115.53		100.5018

				115.55		100.5018

				115.57		100.5018

				115.59		100.5018

				115.61		100.5018

				115.63		100.5078

				115.65		100.5018

				115.68		100.5018

				115.7		100.5018

				115.72		100.5018

				115.74		100.5018

				115.76		100.5018

				115.78		100.5018

				115.8		100.5018

				115.82		100.5018

				115.84		100.5018

				115.86		100.5018

				115.89		100.5018

				115.91		100.5018

				115.93		100.5018

				115.95		100.5018

				115.97		100.5018

				115.99		100.5018

				116.01		100.5018

				116.03		100.5018

				116.05		100.5018

				116.08		100.5018

				116.1		100.5018

				116.12		100.5018

				116.14		100.5018

				116.16		100.5018

				116.18		100.5018

				116.2		100.5018

				116.22		100.5018

				116.24		100.5018

				116.26		100.5018

				116.29		100.5018

				116.31		100.5018

				116.33		100.5018

				116.35		100.5018

				116.37		100.5018

				116.39		100.5018

				116.41		100.5018

				116.43		100.5018

				116.45		100.5018

				116.47		100.5018

				116.5		100.5018

				116.52		100.5018

				116.54		100.5018

				116.56		100.5018

				116.58		100.5018

				116.6		100.5018

				116.62		100.5018

				116.64		100.5018

				116.66		100.5018

				116.68		100.5018

				116.71		100.5018

				116.73		100.5018

				116.75		100.5018

				116.77		100.5018

				116.79		100.5018

				116.81		100.5018

				116.83		100.5018

				116.85		100.5018

				116.87		100.5018

				116.9		100.5018

				116.92		100.5018

				116.94		100.5018

				116.96		100.5018

				116.98		100.5018

				117		100.5018

				117.02		100.5018

				117.04		100.5018

				117.06		100.5018

				117.08		100.5018

				117.11		100.5018

				117.13		100.5018

				117.15		100.5018

				117.17		100.5018

				117.19		100.5018

				117.21		100.5018

				117.23		100.5018

				117.25		100.5018

				117.27		100.5018

				117.29		100.5018

				117.32		100.5018

				117.34		100.5018

				117.36		100.5018

				117.38		100.5018

				117.4		100.5018

				117.42		100.5018

				117.44		100.5018

				117.46		100.5018

				117.48		100.5018

				117.51		100.5018

				117.53		100.5018

				117.55		100.5018

				117.57		100.5018

				117.59		100.5018

				117.61		100.5018

				117.63		100.5018

				117.65		100.5018

				117.67		100.5018

				117.69		100.5018

				117.72		100.5018

				117.74		100.5018

				117.76		100.5018

				117.78		100.5018

				117.8		100.5018

				117.82		100.5018

				117.84		100.5018

				117.86		100.5018

				117.88		100.5018

				117.9		100.5018

				117.93		100.5018

				117.95		100.5018

				117.97		100.5018

				117.99		100.5018

				118.01		100.5018

				118.03		100.5018

				118.05		100.5018

				118.07		100.5018

				118.09		100.5018

				118.11		100.5018

				118.14		100.5018

				118.16		100.5018

				118.18		100.5018

				118.2		100.5018

				118.22		100.5018

				118.24		100.5018

				118.26		100.5018

				118.28		100.5018

				118.3		100.5018

				118.33		100.5018

				118.35		100.5018

				118.37		100.5018

				118.39		100.5018

				118.41		100.5018

				118.43		100.5018

				118.45		100.5018

				118.47		100.5018

				118.49		100.5018

				118.51		100.5018

				118.54		100.5018

				118.56		100.5018

				118.58		100.5018

				118.6		100.5018

				118.62		100.5018

				118.64		100.5018

				118.66		100.5018

				118.68		100.5018

				118.7		100.5018

				118.72		100.5018

				118.75		100.5018

				118.77		100.5018

				118.79		100.5018

				118.81		100.5018

				118.83		100.5018

				118.85		100.5018

				118.87		100.5018

				118.89		100.5018

				118.91		100.5018

				118.93		100.5018

				118.96		100.5018

				118.98		100.5018

				119		100.5018

				119.02		100.5018

				119.04		100.5078

				119.06		100.5018

				119.08		100.5018

				119.1		100.5078

				119.12		100.5078

				119.14		100.5078

				119.17		100.5078

				119.19		100.5078

				119.21		100.5078

				119.23		100.5078

				119.25		100.5078

				119.27		100.5078

				119.29		100.5078

				119.31		100.5078

				119.33		100.5078

				119.36		100.5078

				119.38		100.5078

				119.4		100.5078

				119.42		100.5018

				119.44		100.5018

				119.46		100.5078

				119.48		100.5078

				119.5		100.5078

				119.52		100.5078

				119.54		100.5078

				119.57		100.5078

				119.59		100.5078

				119.61		100.5078

				119.63		100.5078

				119.65		100.5078

				119.67		100.5078

				119.69		100.5078

				119.71		100.5078

				119.73		100.5078

				119.75		100.5018

				119.78		100.5018

				119.8		100.5078

				119.82		100.5018

				119.84		100.5078

				119.86		100.5018

				119.88		100.5018

				119.9		100.5018

				119.92		100.5018

				119.94		100.5018

				119.96		100.5018

				119.99		100.5018

				120.01		100.5018

				120.03		100.5018

				120.05		100.5018

				120.07		100.5018

				120.09		100.5018

				120.11		100.5018

				120.13		100.5018

				120.15		100.5018

				120.17		100.5018

				120.2		100.5018

				120.22		100.5018

				120.24		100.5018

				120.26		100.5018

				120.28		100.5018

				120.3		100.5018

				120.32		100.5018

				120.34		100.5018

				120.36		100.4958

				120.38		100.4958

				120.41		100.4958

				120.43		100.4958

				120.45		100.4958

				120.47		100.4898

				120.49		100.4898

				120.51		100.4958

				120.53		100.4958

				120.55		100.5018

				120.57		100.4958

				120.59		100.4958

				120.62		100.4958

				120.64		100.4958

				120.66		100.4958

				120.68		100.4958

				120.7		100.4958

				120.72		100.4958

				120.74		100.4958

				120.76		100.4958

				120.78		100.4958

				120.8		100.4958

				120.83		100.4958

				120.85		100.4958

				120.87		100.4958

				120.89		100.4898

				120.91		100.4898

				120.93		100.4898

				120.95		100.4898

				120.97		100.4898

				120.99		100.4898

				121.02		100.4898

				121.04		100.4898

				121.06		100.4898

				121.08		100.4898

				121.1		100.4839

				121.12		100.4839

				121.14		100.4839

				121.16		100.4839

				121.18		100.4839

				121.2		100.4839

				121.23		100.4839

				121.25		100.4839

				121.27		100.4839

				121.29		100.4839

				121.31		100.4839

				121.33		100.4839

				121.35		100.4839

				121.37		100.4839

				121.39		100.4839

				121.41		100.4839

				121.44		100.4779

				121.46		100.4839

				121.48		100.4779

				121.5		100.4839

				121.52		100.4779

				121.54		100.4839

				121.56		100.4779

				121.58		100.4779

				121.6		100.4779

				121.62		100.4779

				121.65		100.4779

				121.67		100.4779

				121.69		100.4779

				121.71		100.4779

				121.73		100.4779

				121.75		100.4779

				121.77		100.4779

				121.79		100.4779

				121.81		100.4779

				121.84		100.4779

				121.86		100.4779

				121.88		100.4779

				121.9		100.4779

				121.92		100.4779

				121.94		100.4719

				121.96		100.4719

				121.98		100.4719

				122		100.4719

				122.02		100.4719

				122.05		100.4719

				122.07		100.4719

				122.09		100.4719

				122.11		100.4719

				122.13		100.4719

				122.15		100.4719

				122.17		100.4719

				122.19		100.4719

				122.21		100.4719

				122.23		100.4719

				122.26		100.4719

				122.28		100.4719

				122.3		100.4719

				122.32		100.4719

				122.34		100.4719

				122.36		100.4719

				122.38		100.4719

				122.4		100.4719

				122.42		100.4719

				122.44		100.4719

				122.47		100.4719

				122.49		100.4719

				122.51		100.4719

				122.53		100.4719

				122.55		100.4779

				122.57		100.4779

				122.59		100.4719

				122.61		100.4719

				122.63		100.4659

				122.66		100.4659

				122.68		100.4659

				122.7		100.4659

				122.72		100.4659

				122.74		100.4659

				122.76		100.4719

				122.78		100.4659

				122.8		100.4659

				122.82		100.4659

				122.84		100.4659

				122.87		100.4659

				122.89		100.4659

				122.91		100.4659

				122.93		100.4659

				122.95		100.4659

				122.97		100.4659

				122.99		100.4659

				123.01		100.4659

				123.03		100.4659

				123.06		100.4659

				123.08		100.4659

				123.1		100.4659

				123.12		100.4659

				123.14		100.4659

				123.16		100.4659

				123.18		100.4659

				123.2		100.4659

				123.22		100.4659

				123.24		100.4659

				123.27		100.4659

				123.29		100.4659

				123.31		100.4659

				123.33		100.4659

				123.35		100.4659

				123.37		100.4659

				123.39		100.4659

				123.41		100.4659

				123.43		100.4659

				123.45		100.4659

				123.48		100.4659

				123.5		100.4659

				123.52		100.4659

				123.54		100.4659

				123.56		100.4659

				123.58		100.4659

				123.6		100.4659

				123.62		100.4659

				123.64		100.4659

				123.67		100.4659

				123.69		100.4659

				123.71		100.4659

				123.73		100.4659

				123.75		100.4659

				123.77		100.4659

				123.79		100.4659

				123.81		100.4659

				123.83		100.4659

				123.85		100.4659

				123.88		100.4659

				123.9		100.4659

				123.92		100.4659

				123.94		100.4659

				123.96		100.4659

				123.98		100.4659

				124		100.4659

				124.02		100.4659

				124.04		100.4659

				124.06		100.4659

				124.09		100.4659

				124.11		100.4659

				124.13		100.4659

				124.15		100.4659

				124.17		100.4659

				124.19		100.4659

				124.21		100.4659

				124.23		100.4659

				124.25		100.4659

				124.28		100.4659

				124.3		100.4659

				124.32		100.4659

				124.34		100.4659

				124.36		100.4659

				124.38		100.4659

				124.4		100.46

				124.42		100.46

				124.44		100.4659

				124.46		100.46

				124.49		100.46

				124.51		100.46

				124.53		100.46

				124.55		100.46

				124.57		100.46

				124.59		100.46

				124.61		100.46

				124.63		100.46

				124.65		100.46

				124.68		100.46

				124.7		100.46

				124.72		100.46

				124.74		100.46

				124.76		100.46

				124.78		100.46

				124.8		100.46

				124.82		100.46

				124.84		100.46

				124.86		100.46

				124.89		100.46

				124.91		100.46

				124.93		100.46

				124.95		100.46

				124.97		100.46

				124.99		100.454

				125.01		100.448

				125.03		100.448

				125.05		100.4421

				125.08		100.4421

				125.1		100.4421

				125.12		100.4421

				125.14		100.4421

				125.16		100.4421

				125.18		100.4421

				125.2		100.4421

				125.22		100.4421

				125.24		100.4421

				125.26		100.4421

				125.29		100.4421

				125.31		100.4421

				125.33		100.4421

				125.35		100.4361

				125.37		100.4361

				125.39		100.4361

				125.41		100.4241

				125.43		100.4241

				125.45		100.4241

				125.48		100.4241

				125.5		100.4241

				125.52		100.4241

				125.54		100.4241

				125.56		100.4301

				125.58		100.4301

				125.6		100.4301

				125.62		100.4301

				125.64		100.4361

				125.67		100.4361

				125.69		100.4361

				125.71		100.4421

				125.73		100.448

				125.75		100.454

				125.77		100.46

				125.79		100.4659

				125.81		100.4719

				125.83		100.4719

				125.85		100.4659

				125.88		100.4719

				125.9		100.4719

				125.92		100.4719

				125.94		100.4719

				125.96		100.4719

				125.98		100.4719

				126		100.4659

				126.02		100.4719

				126.04		100.4719

				126.07		100.4719

				126.09		100.4719

				126.11		100.4719

				126.13		100.4719

				126.15		100.4659

				126.17		100.4659

				126.19		100.4659

				126.21		100.4719

				126.23		100.4719

				126.25		100.4719

				126.28		100.4719

				126.3		100.4719

				126.32		100.4719

				126.34		100.4719

				126.36		100.4719

				126.38		100.4719

				126.4		100.4779

				126.42		100.4779

				126.44		100.4779

				126.46		100.4779

				126.49		100.4779

				126.51		100.4779

				126.53		100.4719

				126.55		100.4898

				126.57		100.5197

				126.59		100.5317

				126.61		100.5376

				126.63		100.5376

				126.65		100.5317

				126.68		100.5257

				126.7		100.5197

				126.72		100.5197

				126.74		100.5137

				126.76		100.5137

				126.78		100.5078

				126.8		100.5078

				126.82		100.5078

				126.84		100.5078

				126.87		100.5018

				126.89		100.5018

				126.91		100.5018

				126.93		100.5018

				126.95		100.4958

				126.97		100.4958

				126.99		100.4958

				127.01		100.4958

				127.03		100.4958

				127.05		100.4958

				127.08		100.4958

				127.1		100.4958

				127.12		100.4958

				127.14		100.4958

				127.16		100.4958

				127.18		100.4958

				127.2		100.4958

				127.22		100.5018

				127.24		100.4958

				127.27		100.4958

				127.29		100.4958

				127.31		100.4958

				127.33		100.4898

				127.35		100.4839

				127.37		100.4719

				127.39		100.46

				127.41		100.454

				127.43		100.448

				127.46		100.448

				127.48		100.448

				127.5		100.448

				127.52		100.448

				127.54		100.448

				127.56		100.448

				127.58		100.448

				127.6		100.448

				127.62		100.448

				127.65		100.448

				127.67		100.448

				127.69		100.448

				127.71		100.448

				127.73		100.448

				127.75		100.448

				127.77		100.448

				127.79		100.448

				127.81		100.448

				127.84		100.448

				127.86		100.448

				127.88		100.448

				127.9		100.448

				127.92		100.448

				127.94		100.448

				127.96		100.448

				127.98		100.448

				128		100.448

				128.03		100.448

				128.05		100.448

				128.07		100.448

				128.09		100.448

				128.11		100.448

				128.13		100.448

				128.15		100.448

				128.17		100.448

				128.19		100.448

				128.21		100.448

				128.24		100.448

				128.26		100.454

				128.28		100.454

				128.3		100.448

				128.32		100.454

				128.34		100.454

				128.36		100.454

				128.38		100.454

				128.4		100.448

				128.43		100.448

				128.45		100.448

				128.47		100.448

				128.49		100.448

				128.51		100.448

				128.53		100.448

				128.55		100.448

				128.57		100.448

				128.59		100.448

				128.62		100.448

				128.64		100.448

				128.66		100.4421

				128.68		100.448

				128.7		100.448

				128.72		100.4421

				128.74		100.448

				128.76		100.4421

				128.78		100.4421

				128.81		100.4421

				128.83		100.4421

				128.85		100.4421

				128.87		100.4421

				128.89		100.4421

				128.91		100.4421

				128.93		100.4421

				128.95		100.4421

				128.97		100.4421

				129		100.4421

				129.02		100.4421

				129.04		100.4421

				129.06		100.4421

				129.08		100.4421

				129.1		100.4421

				129.12		100.4421

				129.14		100.4421

				129.16		100.4421

				129.19		100.4421

				129.21		100.4361

				129.23		100.4361

				129.25		100.4361

				129.27		100.4361

				129.29		100.4361

				129.31		100.4361

				129.33		100.4361

				129.35		100.4361

				129.38		100.4361

				129.4		100.4361

				129.42		100.4361

				129.44		100.4361

				129.46		100.4361

				129.48		100.4361

				129.5		100.4361

				129.52		100.4361

				129.54		100.4361

				129.57		100.4301

				129.59		100.4361

				129.61		100.4301

				129.63		100.4301

				129.65		100.4301

				129.67		100.4301

				129.69		100.4301

				129.71		100.4301

				129.73		100.4301

				129.76		100.4301

				129.78		100.4301

				129.8		100.4301

				129.82		100.4301

				129.84		100.4301

				129.86		100.4301

				129.88		100.4301

				129.9		100.4301

				129.92		100.4241

				129.95		100.4241

				129.97		100.4241

				129.99		100.4241

				130.01		100.4241

				130.03		100.4241

				130.05		100.4241

				130.07		100.4241

				130.09		100.4241

				130.11		100.4241

				130.14		100.4241

				130.16		100.4241

				130.18		100.4241

				130.2		100.4241

				130.22		100.4241

				130.24		100.4241

				130.26		100.4241

				130.28		100.4241

				130.3		100.4241

				130.33		100.4241

				130.35		100.4241

				130.37		100.4241

				130.39		100.4241

				130.41		100.4182

				130.43		100.4182

				130.45		100.4182

				130.47		100.4182

				130.49		100.4182

				130.52		100.4182

				130.54		100.4182

				130.56		100.4182

				130.58		100.4182

				130.6		100.4241

				130.62		100.4241

				130.64		100.4241

				130.66		100.4241

				130.68		100.4241

				130.71		100.4241

				130.73		100.4241

				130.75		100.4241

				130.77		100.4241

				130.79		100.4241

				130.81		100.4241

				130.83		100.4241

				130.85		100.4241

				130.87		100.4241

				130.9		100.4182

				130.92		100.4182

				130.94		100.4182

				130.96		100.4182

				130.98		100.4182

				131		100.4182

				131.02		100.4182

				131.04		100.4182

				131.06		100.4182

				131.09		100.4182

				131.11		100.4182

				131.13		100.4182

				131.15		100.4182

				131.17		100.4182

				131.19		100.4182

				131.21		100.4182

				131.23		100.4182

				131.25		100.4182

				131.28		100.4182

				131.3		100.4182

				131.32		100.4182

				131.34		100.4182

				131.36		100.4182

				131.38		100.4182

				131.4		100.4182

				131.42		100.4182

				131.44		100.4182

				131.47		100.4182

				131.49		100.4182

				131.51		100.4182

				131.53		100.4182

				131.55		100.4182

				131.57		100.4182

				131.59		100.4182

				131.61		100.4182

				131.63		100.4182

				131.66		100.4182

				131.68		100.4182

				131.7		100.4182

				131.72		100.4122

				131.74		100.4122

				131.76		100.4122

				131.78		100.4122

				131.8		100.4122

				131.82		100.4122

				131.85		100.4122

				131.87		100.4122

				131.89		100.4122

				131.91		100.4122

				131.93		100.4122

				131.95		100.4122

				131.97		100.4122

				131.99		100.4122

				132.01		100.4122

				132.04		100.4122

				132.06		100.4122

				132.08		100.4122

				132.1		100.4122

				132.12		100.4122

				132.14		100.4122

				132.16		100.4122

				132.18		100.4122

				132.2		100.4122

				132.23		100.4122

				132.25		100.4122

				132.27		100.4122

				132.29		100.4122

				132.31		100.4122

				132.33		100.4122

				132.35		100.4122

				132.37		100.4062

				132.39		100.4062

				132.42		100.4062

				132.44		100.4062

				132.46		100.4062

				132.48		100.4062

				132.5		100.4062

				132.52		100.4062

				132.54		100.4062

				132.56		100.4062

				132.58		100.4062

				132.61		100.4062

				132.63		100.4062

				132.65		100.4062

				132.67		100.4062

				132.69		100.4062

				132.71		100.4062

				132.73		100.4062

				132.75		100.4062

				132.78		100.4062

				132.8		100.4062

				132.82		100.4062

				132.84		100.4062

				132.86		100.4062

				132.88		100.4062

				132.9		100.4062

				132.92		100.4002

				132.94		100.4002

				132.97		100.4002

				132.99		100.4002

				133.01		100.4002

				133.03		100.4002

				133.05		100.4002

				133.07		100.4002

				133.09		100.4002

				133.11		100.4002

				133.13		100.4002

				133.16		100.4002

				133.18		100.4002

				133.2		100.4002

				133.22		100.4002

				133.24		100.4002

				133.26		100.4002

				133.28		100.4002

				133.3		100.4002

				133.32		100.4002

				133.35		100.3943

				133.37		100.3943

				133.39		100.3943

				133.41		100.3943

				133.43		100.3943

				133.45		100.3943

				133.47		100.3943

				133.49		100.3943

				133.51		100.3943

				133.54		100.3943

				133.56		100.3943

				133.58		100.3943

				133.6		100.3943

				133.62		100.3943

				133.64		100.3943

				133.66		100.3943

				133.68		100.3943

				133.7		100.3943

				133.73		100.3943

				133.75		100.3943

				133.77		100.3943

				133.79		100.3943

				133.81		100.3943

				133.83		100.3943

				133.85		100.3943

				133.87		100.3943

				133.89		100.3883

				133.92		100.3883

				133.94		100.3883

				133.96		100.3883

				133.98		100.3883

				134		100.3883

				134.02		100.3883

				134.04		100.3883

				134.06		100.3883

				134.08		100.3883

				134.11		100.3883

				134.13		100.3883

				134.15		100.3883

				134.17		100.3883

				134.19		100.3883

				134.21		100.3883

				134.23		100.3883

				134.25		100.3883

				134.27		100.3883

				134.3		100.3883

				134.32		100.3883

				134.34		100.3823

				134.36		100.3823

				134.38		100.3823

				134.4		100.3823

				134.42		100.3823

				134.44		100.3823

				134.47		100.3823

				134.49		100.3823

				134.51		100.3823

				134.53		100.3823

				134.55		100.3823

				134.57		100.3763

				134.59		100.3763

				134.61		100.3763

				134.63		100.3763

				134.66		100.3763

				134.68		100.3763

				134.7		100.3763

				134.72		100.3763

				134.74		100.3763

				134.76		100.3763

				134.78		100.3763

				134.8		100.3763

				134.82		100.3763

				134.85		100.3763

				134.87		100.3704

				134.89		100.3704

				134.91		100.3704

				134.93		100.3704

				134.95		100.3704

				134.97		100.3704

				134.99		100.3704

				135.01		100.3704

				135.04		100.3704

				135.06		100.3704

				135.08		100.3704

				135.1		100.3644

				135.12		100.3704

				135.14		100.3644

				135.16		100.3644

				135.18		100.3644

				135.2		100.3644

				135.23		100.3644

				135.25		100.3644

				135.27		100.3644

				135.29		100.3644

				135.31		100.3644

				135.33		100.3644

				135.35		100.3644

				135.37		100.3644

				135.4		100.3584

				135.42		100.3584

				135.44		100.3584

				135.46		100.3584

				135.48		100.3584

				135.5		100.3584

				135.52		100.3584

				135.54		100.3584

				135.56		100.3584

				135.59		100.3584

				135.61		100.3584

				135.63		100.3584

				135.65		100.3584

				135.67		100.3584

				135.69		100.3584

				135.71		100.3584

				135.73		100.3584

				135.75		100.3524

				135.78		100.3584

				135.8		100.3524

				135.82		100.3524

				135.84		100.3524

				135.86		100.3524

				135.88		100.3524

				135.9		100.3524

				135.92		100.3524

				135.95		100.3524

				135.97		100.3524

				135.99		100.3524

				136.01		100.3524

				136.03		100.3465

				136.05		100.3465

				136.07		100.3465

				136.09		100.3465

				136.11		100.3465

				136.14		100.3465

				136.16		100.3465

				136.18		100.3465

				136.2		100.3465

				136.22		100.3465

				136.24		100.3465

				136.26		100.3405

				136.28		100.3405

				136.3		100.3405

				136.33		100.3405

				136.35		100.3405

				136.37		100.3405

				136.39		100.3405

				136.41		100.3405

				136.43		100.3405

				136.45		100.3405

				136.47		100.3405

				136.5		100.3405

				136.52		100.3405

				136.54		100.3405

				136.56		100.3405

				136.58		100.3345

				136.6		100.3345

				136.62		100.3345

				136.64		100.3345

				136.66		100.3345

				136.69		100.3345

				136.71		100.3345

				136.73		100.3345

				136.75		100.3345

				136.77		100.3345

				136.79		100.3286

				136.81		100.3286

				136.83		100.3286

				136.85		100.3286

				136.88		100.3286

				136.9		100.3286

				136.92		100.3286

				136.94		100.3286

				136.96		100.3286

				136.98		100.3286

				137		100.3286

				137.02		100.3286

				137.05		100.3286

				137.07		100.3286

				137.09		100.3286

				137.11		100.3226

				137.13		100.3226

				137.15		100.3226

				137.17		100.3226

				137.19		100.3226

				137.21		100.3226

				137.24		100.3226

				137.26		100.3226

				137.28		100.3226

				137.3		100.3226

				137.32		100.3226

				137.34		100.3226

				137.36		100.3226

				137.38		100.3226

				137.4		100.3226

				137.43		100.3226

				137.45		100.3226

				137.47		100.3226

				137.49		100.3226

				137.51		100.3166

				137.53		100.3166

				137.55		100.3166

				137.57		100.3166

				137.59		100.3226

				137.62		100.3226

				137.64		100.3166

				137.66		100.3166

				137.68		100.3166

				137.7		100.3166

				137.72		100.3166

				137.74		100.3166

				137.76		100.3166

				137.79		100.3166

				137.81		100.3166

				137.83		100.3166

				137.85		100.3106

				137.87		100.3106

				137.89		100.3106

				137.91		100.3106

				137.93		100.3106

				137.95		100.3106

				137.98		100.3106

				138		100.3106

				138.02		100.3106

				138.04		100.3106

				138.06		100.3106

				138.08		100.3106

				138.1		100.3106

				138.12		100.3106

				138.14		100.3106

				138.17		100.3106

				138.19		100.3106

				138.21		100.3106

				138.23		100.3106

				138.25		100.3106

				138.27		100.3106

				138.29		100.3106

				138.31		100.3106

				138.33		100.3106

				138.36		100.3106

				138.38		100.3047

				138.4		100.3047

				138.42		100.3047

				138.44		100.3047

				138.46		100.3047

				138.48		100.3047

				138.5		100.3047

				138.53		100.3047

				138.55		100.3047

				138.57		100.3047

				138.59		100.3047

				138.61		100.2987

				138.63		100.2987

				138.65		100.2987

				138.67		100.2987

				138.69		100.2987

				138.72		100.2987

				138.74		100.2987

				138.76		100.2987

				138.78		100.2987

				138.8		100.2987

				138.82		100.2987

				138.84		100.2987

				138.86		100.2987

				138.88		100.2987

				138.91		100.2987

				138.93		100.2927

				138.95		100.2927

				138.97		100.2927

				138.99		100.2927

				139.01		100.2927

				139.03		100.2927

				139.05		100.2927

				139.08		100.2927

				139.1		100.2927

				139.12		100.2927

				139.14		100.2927

				139.16		100.2927

				139.18		100.2927

				139.2		100.2927

				139.22		100.2927

				139.24		100.2927

				139.27		100.2927

				139.29		100.2927

				139.31		100.2927

				139.33		100.2867

				139.35		100.2927

				139.37		100.2867

				139.39		100.2867

				139.41		100.2867

				139.43		100.2867

				139.46		100.2867

				139.48		100.2867

				139.5		100.2867

				139.52		100.2867

				139.54		100.2867

				139.56		100.2867

				139.58		100.2808

				139.6		100.2808

				139.63		100.2808

				139.65		100.2808

				139.67		100.2808

				139.69		100.2808

				139.71		100.2808

				139.73		100.2808

				139.75		100.2808

				139.77		100.2808

				139.79		100.2808

				139.82		100.2808

				139.84		100.2808

				139.86		100.2808

				139.88		100.2808

				139.9		100.2808

				139.92		100.2748

				139.94		100.2748

				139.96		100.2748

				139.99		100.2748

				140.01		100.2748

				140.03		100.2748

				140.05		100.2748

				140.07		100.2748

				140.09		100.2688

				140.11		100.2688

				140.13		100.2688

				140.15		100.2688

				140.18		100.2688

				140.2		100.2688

				140.22		100.2688

				140.24		100.2688

				140.26		100.2628

				140.28		100.2628

				140.3		100.2628

				140.32		100.2628

				140.35		100.2628

				140.37		100.2628

				140.39		100.2628

				140.41		100.2628

				140.43		100.2628

				140.45		100.2628

				140.47		100.2628

				140.49		100.2628

				140.51		100.2628

				140.54		100.2628

				140.56		100.2628

				140.58		100.2628

				140.6		100.2628

				140.62		100.2628

				140.64		100.2628

				140.66		100.2628

				140.68		100.2628

				140.7		100.2628

				140.73		100.2569

				140.75		100.2569

				140.77		100.2569

				140.79		100.2569

				140.81		100.2569

				140.83		100.2569

				140.85		100.2569

				140.87		100.2569

				140.9		100.2569

				140.92		100.2569

				140.94		100.2569

				140.96		100.2569

				140.98		100.2569

				141		100.2569

				141.02		100.2569

				141.04		100.2569

				141.06		100.2569

				141.09		100.2509

				141.11		100.2509

				141.13		100.2509

				141.15		100.2509

				141.17		100.2509

				141.19		100.2509

				141.21		100.2509

				141.23		100.2509

				141.25		100.2509

				141.28		100.2509

				141.3		100.2509

				141.32		100.2509

				141.34		100.2509

				141.36		100.2509

				141.38		100.2509

				141.4		100.2509

				141.42		100.2509

				141.45		100.2509

				141.47		100.2449

				141.49		100.2449

				141.51		100.2449

				141.53		100.2449

				141.55		100.2449

				141.57		100.2449

				141.59		100.2449

				141.61		100.2449

				141.64		100.2449

				141.66		100.2449

				141.68		100.2389

				141.7		100.2389

				141.72		100.2389

				141.74		100.2389

				141.76		100.2389

				141.78		100.2389

				141.81		100.2389

				141.83		100.2389

				141.85		100.2389

				141.87		100.233

				141.89		100.233

				141.91		100.233

				141.93		100.233

				141.95		100.233

				141.97		100.233

				142		100.233

				142.02		100.233

				142.04		100.233

				142.06		100.233

				142.08		100.233

				142.1		100.233

				142.12		100.233

				142.14		100.233

				142.17		100.233

				142.19		100.227

				142.21		100.227

				142.23		100.227

				142.25		100.227

				142.27		100.227

				142.29		100.227

				142.31		100.227

				142.33		100.227

				142.36		100.227

				142.38		100.227

				142.4		100.221

				142.42		100.221

				142.44		100.221

				142.46		100.221

				142.48		100.221

				142.5		100.221

				142.53		100.221

				142.55		100.221

				142.57		100.221

				142.59		100.2151

				142.61		100.2151

				142.63		100.2151

				142.65		100.2151

				142.67		100.2151

				142.69		100.2151

				142.72		100.2151

				142.74		100.2151

				142.76		100.2151

				142.78		100.2151

				142.8		100.2091

				142.82		100.2091

				142.84		100.2091

				142.86		100.2091

				142.89		100.2091

				142.91		100.2091

				142.93		100.2091

				142.95		100.2091

				142.97		100.2031

				142.99		100.2031

				143.01		100.2031

				143.03		100.2031

				143.05		100.2031

				143.08		100.2031

				143.1		100.2031

				143.12		100.1971

				143.14		100.1971

				143.16		100.1971

				143.18		100.1971

				143.2		100.2031

				143.22		100.2031

				143.24		100.2031

				143.27		100.1971

				143.29		100.2031

				143.31		100.1971

				143.33		100.1971

				143.35		100.1971

				143.37		100.1971

				143.39		100.1971

				143.41		100.1971

				143.44		100.1971

				143.46		100.1971

				143.48		100.1971

				143.5		100.1971

				143.52		100.1971

				143.54		100.1971

				143.56		100.1971

				143.58		100.1971

				143.61		100.1971

				143.63		100.1971

				143.65		100.1971

				143.67		100.1971

				143.69		100.1971

				143.71		100.1912

				143.73		100.1912

				143.75		100.1912

				143.77		100.1912

				143.8		100.1912

				143.82		100.1912

				143.84		100.1912

				143.86		100.1912

				143.88		100.1912

				143.9		100.1912

				143.92		100.1912

				143.94		100.1912

				143.97		100.1852

				143.99		100.1852

				144.01		100.1852

				144.03		100.1852

				144.05		100.1852

				144.07		100.1852

				144.09		100.1852

				144.11		100.1852

				144.13		100.1852

				144.16		100.1852

				144.18		100.1852

				144.2		100.1852

				144.22		100.1852

				144.24		100.1852

				144.26		100.1852

				144.28		100.1792

				144.3		100.1792

				144.33		100.1792

				144.35		100.1792

				144.37		100.1792

				144.39		100.1792

				144.41		100.1792

				144.43		100.1792

				144.45		100.1792

				144.47		100.1792

				144.49		100.1792

				144.52		100.1792

				144.54		100.1792

				144.56		100.1792

				144.58		100.1792

				144.6		100.1792

				144.62		100.1732

				144.64		100.1732

				144.66		100.1732

				144.69		100.1792

				144.71		100.1732

				144.73		100.1732

				144.75		100.1732

				144.77		100.1732

				144.79		100.1732

				144.81		100.1732

				144.83		100.1732

				144.86		100.1732

				144.88		100.1732

				144.9		100.1732

				144.92		100.1732

				144.94		100.1673

				144.96		100.1673

				144.98		100.1673

				145		100.1673

				145.02		100.1673

				145.05		100.1613

				145.07		100.1613

				145.09		100.1613

				145.11		100.1613

				145.13		100.1613

				145.15		100.1613

				145.17		100.1613

				145.19		100.1553

				145.22		100.1553

				145.24		100.1553

				145.26		100.1553

				145.28		100.1553

				145.3		100.1553

				145.32		100.1493

				145.34		100.1493

				145.36		100.1493

				145.39		100.1493

				145.41		100.1493

				145.43		100.1434

				145.45		100.1434

				145.47		100.1434

				145.49		100.1434

				145.51		100.1434

				145.53		100.1434

				145.55		100.1374

				145.58		100.1374

				145.6		100.1374

				145.62		100.1374

				145.64		100.1374

				145.66		100.1374

				145.68		100.1374

				145.7		100.1374

				145.72		100.1374

				145.75		100.1374

				145.77		100.1314

				145.79		100.1314

				145.81		100.1314

				145.83		100.1314

				145.85		100.1314

				145.87		100.1314

				145.89		100.1314

				145.91		100.1254

				145.94		100.1254

				145.96		100.1254

				145.98		100.1254

				146		100.1254

				146.02		100.1254

				146.04		100.1254

				146.06		100.1254

				146.08		100.1254

				146.11		100.1254

				146.13		100.1254

				146.15		100.1254

				146.17		100.1195

				146.19		100.1195

				146.21		100.1195

				146.23		100.1195

				146.25		100.1195

				146.27		100.1195

				146.3		100.1195

				146.32		100.1195

				146.34		100.1135

				146.36		100.1135

				146.38		100.1135

				146.4		100.1135

				146.42		100.1135

				146.44		100.1135

				146.47		100.1135

				146.49		100.1135

				146.51		100.1135

				146.53		100.1075

				146.55		100.1075

				146.57		100.1075

				146.59		100.1075

				146.61		100.1075

				146.64		100.1075

				146.66		100.1075

				146.68		100.1075

				146.7		100.1075

				146.72		100.1075

				146.74		100.1016

				146.76		100.1016

				146.78		100.1016

				146.8		100.1016

				146.83		100.1016

				146.85		100.1016

				146.87		100.1016

				146.89		100.1016

				146.91		100.1016

				146.93		100.1016

				146.95		100.1016

				146.97		100.1016

				147		100.1016

				147.02		100.0956

				147.04		100.0956

				147.06		100.0956

				147.08		100.0956

				147.1		100.0956

				147.12		100.0956

				147.14		100.0956

				147.17		100.0956

				147.19		100.0956

				147.21		100.0956

				147.23		100.0956

				147.25		100.0896

				147.27		100.0896

				147.29		100.0896

				147.31		100.0896

				147.33		100.0896

				147.36		100.0896

				147.38		100.0896

				147.4		100.0896

				147.42		100.0896

				147.44		100.0896

				147.46		100.0896

				147.48		100.0896

				147.5		100.0896

				147.53		100.0836

				147.55		100.0836

				147.57		100.0836

				147.59		100.0836

				147.61		100.0836

				147.63		100.0836

				147.65		100.0836

				147.67		100.0836

				147.69		100.0777

				147.72		100.0777

				147.74		100.0777

				147.76		100.0777

				147.78		100.0777

				147.8		100.0777

				147.82		100.0777

				147.84		100.0777

				147.86		100.0777

				147.89		100.0777

				147.91		100.0777

				147.93		100.0777

				147.95		100.0717

				147.97		100.0717

				147.99		100.0717

				148.01		100.0717

				148.03		100.0717

				148.05		100.0717

				148.08		100.0717

				148.1		100.0717

				148.12		100.0657

				148.14		100.0657

				148.16		100.0657

				148.18		100.0657

				148.2		100.0657

				148.22		100.0657

				148.25		100.0657

				148.27		100.0657

				148.29		100.0657

				148.31		100.0657

				148.33		100.0657

				148.35		100.0657

				148.37		100.0657

				148.39		100.0657

				148.41		100.0657

				148.44		100.0597

				148.46		100.0597

				148.48		100.0597

				148.5		100.0597

				148.52		100.0597

				148.54		100.0597

				148.56		100.0597

				148.58		100.0597

				148.61		100.0597

				148.63		100.0538

				148.65		100.0538

				148.67		100.0538

				148.69		100.0538

				148.71		100.0538

				148.73		100.0538

				148.75		100.0538

				148.77		100.0538

				148.8		100.0478

				148.82		100.0478

				148.84		100.0478

				148.86		100.0478

				148.88		100.0478

				148.9		100.0478

				148.92		100.0478

				148.94		100.0478

				148.97		100.0418

				148.99		100.0418

				149.01		100.0418

				149.03		100.0418

				149.05		100.0418

				149.07		100.0418

				149.09		100.0418

				149.11		100.0418

				149.13		100.0358

				149.16		100.0358

				149.18		100.0358

				149.2		100.0358

				149.22		100.0358

				149.24		100.0358

				149.26		100.0358

				149.28		100.0358

				149.3		100.0299

				149.33		100.0299

				149.35		100.0299

				149.37		100.0299

				149.39		100.0299

				149.41		100.0299

				149.43		100.0299

				149.45		100.0299

				149.47		100.0239

				149.49		100.0239

				149.52		100.0239

				149.54		100.0239

				149.56		100.0239

				149.58		100.0179

				149.6		100.0179

				149.62		100.0179

				149.64		100.0179

				149.66		100.0179

				149.69		100.0179

				149.71		100.0179

				149.73		100.0119

				149.75		100.0119

				149.77		100.0119

				149.79		100.0119

				149.81		100.0119

				149.83		100.006

				149.85		100.006

				149.88		100.006

				149.9		100.006

				149.92		100

				149.94		100

				149.96		100

				149.98		99.99403

				150		99.99403

				150.02		99.99403

				150.05		99.99403

				150.07		99.98805

				150.09		99.98805

				150.11		99.98805

				150.13		99.98805

				150.15		99.98805

				150.17		99.98208

				150.19		99.98208

				150.21		99.98208

				150.24		99.98208

				150.26		99.98208

				150.28		99.98208

				150.3		99.97611

				150.32		99.97611

				150.34		99.97611

				150.36		99.97611

				150.38		99.97013

				150.41		99.97013

				150.43		99.96416

				150.45		99.96416

				150.47		99.96416

				150.49		99.96416

				150.51		99.96416

				150.53		99.96416

				150.55		99.95818

				150.57		99.95818

				150.6		99.95818

				150.62		99.95818

				150.64		99.95818

				150.66		99.95818

				150.68		99.95221

				150.7		99.95221

				150.72		99.95221

				150.74		99.95221

				150.77		99.94624

				150.79		99.94624

				150.81		99.94624

				150.83		99.94624

				150.85		99.94624

				150.87		99.94624

				150.89		99.94624

				150.91		99.94624

				150.93		99.94624

				150.96		99.94624

				150.98		99.94624

				151		99.94624

				151.02		99.94624

				151.04		99.94624

				151.06		99.94624

				151.08		99.94624

				151.1		99.94026

				151.13		99.94026

				151.15		99.94026

				151.17		99.94026

				151.19		99.94026

				151.21		99.94026

				151.23		99.93429

				151.25		99.93429

				151.27		99.93429

				151.29		99.93429

				151.32		99.93429

				151.34		99.93429

				151.36		99.93429

				151.38		99.92832

				151.4		99.92832

				151.42		99.92832

				151.44		99.92832

				151.46		99.92832

				151.49		99.92832

				151.51		99.92832

				151.53		99.92234

				151.55		99.92234

				151.57		99.92234

				151.59		99.92234

				151.61		99.92234

				151.63		99.92234

				151.65		99.92234

				151.68		99.92234

				151.7		99.91637

				151.72		99.91637

				151.74		99.91637

				151.76		99.91637

				151.78		99.91637

				151.8		99.91637

				151.82		99.91637

				151.85		99.91637

				151.87		99.91637

				151.89		99.91637

				151.91		99.91039

				151.93		99.91039

				151.95		99.91039

				151.97		99.91039

				151.99		99.91039

				152.01		99.90442

				152.04		99.91039

				152.06		99.90442

				152.08		99.90442

				152.1		99.90442

				152.12		99.90442

				152.14		99.90442

				152.16		99.90442

				152.18		99.90442

				152.2		99.89845

				152.23		99.89845

				152.25		99.89845

				152.27		99.89845

				152.29		99.89845

				152.31		99.89845

				152.33		99.89247

				152.35		99.89247

				152.37		99.89247

				152.4		99.89247

				152.42		99.8865

				152.44		99.8865

				152.46		99.8865

				152.48		99.88053

				152.5		99.88053

				152.52		99.88053

				152.54		99.88053

				152.56		99.88053

				152.59		99.88053

				152.61		99.88053

				152.63		99.87455

				152.65		99.87455

				152.67		99.87455

				152.69		99.87455

				152.71		99.87455

				152.73		99.87455

				152.75		99.87455

				152.78		99.86858

				152.8		99.86858

				152.82		99.86858

				152.84		99.86858

				152.86		99.86858

				152.88		99.86858

				152.9		99.8626

				152.92		99.8626

				152.95		99.8626

				152.97		99.8626

				152.99		99.8626

				153.01		99.8626

				153.03		99.85663

				153.05		99.85663

				153.07		99.85663

				153.09		99.85663

				153.12		99.85663

				153.14		99.85066

				153.16		99.85066

				153.18		99.85066

				153.2		99.85066

				153.22		99.85066

				153.24		99.84468

				153.26		99.84468

				153.28		99.84468

				153.31		99.84468

				153.33		99.84468

				153.35		99.84468

				153.37		99.83871

				153.39		99.83871

				153.41		99.83871

				153.43		99.83871

				153.45		99.83871

				153.48		99.83871

				153.5		99.83871

				153.52		99.83274

				153.54		99.83274

				153.56		99.83274

				153.58		99.83274

				153.6		99.83274

				153.62		99.82676

				153.64		99.82676

				153.67		99.82676

				153.69		99.82676

				153.71		99.82676

				153.73		99.82079

				153.75		99.82079

				153.77		99.82079

				153.79		99.82079

				153.81		99.82079

				153.83		99.81481

				153.86		99.81481

				153.88		99.81481

				153.9		99.81481

				153.92		99.81481

				153.94		99.80884

				153.96		99.80884

				153.98		99.80884

				154		99.80884

				154.03		99.80884

				154.05		99.80884

				154.07		99.80884

				154.09		99.80287

				154.11		99.80287

				154.13		99.80287

				154.15		99.80287

				154.17		99.80287

				154.19		99.80287

				154.22		99.80287

				154.24		99.79689

				154.26		99.79689

				154.28		99.79689

				154.3		99.79689

				154.32		99.79689

				154.34		99.79092

				154.36		99.79092

				154.39		99.79092

				154.41		99.79092

				154.43		99.79092

				154.45		99.79092

				154.47		99.78495

				154.49		99.78495

				154.51		99.78495

				154.53		99.78495

				154.55		99.78495

				154.58		99.77897

				154.6		99.77897

				154.62		99.77897

				154.64		99.77897

				154.66		99.77897

				154.68		99.77897

				154.7		99.77897

				154.72		99.773

				154.75		99.773

				154.77		99.773

				154.79		99.773

				154.81		99.773

				154.83		99.773

				154.85		99.773

				154.87		99.76703

				154.89		99.76703

				154.91		99.76703

				154.94		99.76703

				154.96		99.76105

				154.98		99.76105

				155		99.76105

				155.02		99.76105

				155.04		99.76105

				155.06		99.76105

				155.08		99.75508

				155.1		99.75508

				155.13		99.75508

				155.15		99.75508

				155.17		99.75508

				155.19		99.75508

				155.21		99.7491

				155.23		99.7491

				155.25		99.7491

				155.27		99.74313

				155.3		99.74313

				155.32		99.74313

				155.34		99.74313

				155.36		99.74313

				155.38		99.73716

				155.4		99.73716

				155.42		99.73716

				155.44		99.73716

				155.46		99.73118

				155.49		99.73118

				155.51		99.73118

				155.53		99.72521

				155.55		99.72521

				155.57		99.72521

				155.59		99.72521

				155.61		99.72521

				155.63		99.71924

				155.66		99.71924

				155.68		99.71924

				155.7		99.71924

				155.72		99.71326

				155.74		99.71326

				155.76		99.71326

				155.78		99.71326

				155.8		99.70729

				155.82		99.70729

				155.85		99.70729

				155.87		99.70729

				155.89		99.70729

				155.91		99.70729

				155.93		99.70131

				155.95		99.70131

				155.97		99.70131

				155.99		99.70131

				156.02		99.70131

				156.04		99.70131

				156.06		99.69534

				156.08		99.69534

				156.1		99.69534

				156.12		99.69534

				156.14		99.69534

				156.16		99.69534

				156.18		99.68937

				156.21		99.69534

				156.23		99.68937

				156.25		99.68937

				156.27		99.68937

				156.29		99.68937

				156.31		99.68937

				156.33		99.68339

				156.35		99.68339

				156.37		99.68339

				156.4		99.68339

				156.42		99.68339

				156.44		99.67742

				156.46		99.67742

				156.48		99.67742

				156.5		99.67742

				156.52		99.67742

				156.54		99.67145

				156.57		99.67145

				156.59		99.67145

				156.61		99.67145

				156.63		99.67145

				156.65		99.67145

				156.67		99.67145

				156.69		99.66547

				156.71		99.66547

				156.73		99.66547

				156.76		99.66547

				156.78		99.66547

				156.8		99.66547

				156.82		99.6595

				156.84		99.6595

				156.86		99.6595

				156.88		99.6595

				156.9		99.6595

				156.92		99.6595

				156.95		99.6595

				156.97		99.65352

				156.99		99.65352

				157.01		99.65352

				157.03		99.65352

				157.05		99.65352

				157.07		99.64755

				157.09		99.64755

				157.12		99.64755

				157.14		99.64755

				157.16		99.64755

				157.18		99.64158

				157.2		99.64158

				157.22		99.6356

				157.24		99.6356

				157.26		99.6356

				157.28		99.62963

				157.31		99.62963

				157.33		99.62963

				157.35		99.62963

				157.37		99.62963

				157.39		99.62366

				157.41		99.62366

				157.43		99.62366

				157.45		99.62366

				157.47		99.61768

				157.5		99.61768

				157.52		99.61768

				157.54		99.61768

				157.56		99.61171

				157.58		99.61171

				157.6		99.61171

				157.62		99.61171

				157.64		99.61171

				157.66		99.61171

				157.69		99.61171

				157.71		99.60573

				157.73		99.60573

				157.75		99.60573

				157.77		99.60573

				157.79		99.59976

				157.81		99.59976

				157.83		99.59379

				157.85		99.59379

				157.88		99.58781

				157.9		99.58781

				157.92		99.58781

				157.94		99.58781

				157.96		99.58781

				157.98		99.58781

				158		99.58184

				158.02		99.58184

				158.04		99.58184

				158.07		99.57587

				158.09		99.57587

				158.11		99.57587

				158.13		99.57587

				158.15		99.57587

				158.17		99.56989

				158.19		99.56989

				158.21		99.56392

				158.23		99.56989

				158.26		99.56392

				158.28		99.56392

				158.3		99.56392

				158.32		99.56392

				158.34		99.55795

				158.36		99.55795

				158.38		99.55795

				158.4		99.55197

				158.43		99.55197

				158.45		99.55197

				158.47		99.55197

				158.49		99.55197

				158.51		99.546

				158.53		99.546

				158.55		99.546

				158.57		99.546

				158.59		99.546

				158.62		99.546

				158.64		99.54002

				158.66		99.54002

				158.68		99.54002

				158.7		99.54002

				158.72		99.54002

				158.74		99.53405

				158.76		99.53405

				158.78		99.53405

				158.81		99.53405

				158.83		99.53405

				158.85		99.52808

				158.87		99.52808

				158.89		99.52808

				158.91		99.52808

				158.93		99.5221

				158.95		99.5221

				158.97		99.5221

				159		99.5221

				159.02		99.51613

				159.04		99.51613

				159.06		99.51613

				159.08		99.51613

				159.1		99.51016

				159.12		99.51016

				159.14		99.51016

				159.16		99.50418

				159.19		99.50418

				159.21		99.50418

				159.23		99.50418

				159.25		99.50418

				159.27		99.49821

				159.29		99.49821

				159.31		99.49821

				159.33		99.49821

				159.36		99.49821

				159.38		99.49821

				159.4		99.49223

				159.42		99.49223

				159.44		99.49223

				159.46		99.48626

				159.48		99.48626

				159.5		99.48626

				159.52		99.48029

				159.55		99.48029

				159.57		99.48029

				159.59		99.47431

				159.61		99.47431

				159.63		99.47431

				159.65		99.47431

				159.67		99.47431

				159.69		99.47431

				159.71		99.47431

				159.74		99.46834

				159.76		99.46834

				159.78		99.46834

				159.8		99.46237

				159.82		99.46237

				159.84		99.46237

				159.86		99.46237

				159.88		99.45639

				159.91		99.45639

				159.93		99.45639

				159.95		99.45639

				159.97		99.45639

				159.99		99.45639

				160.01		99.45639

				160.03		99.45639

				160.05		99.45042

				160.07		99.45042

				160.1		99.45042

				160.12		99.45042

				160.14		99.45042

				160.16		99.45042

				160.18		99.45042

				160.2		99.44444

				160.22		99.44444

				160.24		99.44444

				160.26		99.43847

				160.29		99.43847

				160.31		99.43847

				160.33		99.43847

				160.35		99.4325

				160.37		99.4325

				160.39		99.4325

				160.41		99.4325

				160.43		99.4325

				160.45		99.4325

				160.47		99.42652

				160.5		99.42652

				160.52		99.42652

				160.54		99.42652

				160.56		99.42055

				160.58		99.42055

				160.6		99.42055

				160.62		99.42055

				160.64		99.42055

				160.66		99.41458

				160.69		99.41458

				160.71		99.41458

				160.73		99.4086

				160.75		99.4086

				160.77		99.4086

				160.79		99.40263

				160.81		99.40263

				160.83		99.40263

				160.85		99.40263

				160.88		99.39665

				160.9		99.39665

				160.92		99.39068

				160.94		99.39068

				160.96		99.39068

				160.98		99.39068

				161		99.39068

				161.02		99.38471

				161.04		99.38471

				161.07		99.38471

				161.09		99.38471

				161.11		99.37873

				161.13		99.37873

				161.15		99.37873

				161.17		99.37873

				161.19		99.37276

				161.21		99.37276

				161.23		99.37276

				161.26		99.36679

				161.28		99.36679

				161.3		99.36679

				161.32		99.36679

				161.34		99.36679

				161.36		99.36679

				161.38		99.36679

				161.4		99.36081

				161.42		99.36081

				161.45		99.36081

				161.47		99.36081

				161.49		99.36081

				161.51		99.36081

				161.53		99.35484

				161.55		99.35484

				161.57		99.35484

				161.59		99.34886

				161.62		99.35484

				161.64		99.34886

				161.66		99.34886

				161.68		99.34886

				161.7		99.34886

				161.72		99.34289

				161.74		99.34289

				161.76		99.34289

				161.78		99.34289

				161.81		99.33692

				161.83		99.33094

				161.85		99.33094

				161.87		99.33094

				161.89		99.32497

				161.91		99.32497

				161.93		99.319

				161.95		99.319

				161.97		99.319

				161.99		99.31302

				162.02		99.31302

				162.04		99.31302

				162.06		99.30705

				162.08		99.30108

				162.1		99.30108

				162.12		99.2951

				162.14		99.2951

				162.16		99.28913

				162.18		99.28913

				162.21		99.28315

				162.23		99.28315

				162.25		99.27718

				162.27		99.27718

				162.29		99.27121

				162.31		99.27121

				162.33		99.26523

				162.35		99.26523

				162.37		99.25926

				162.4		99.25926

				162.42		99.25926

				162.44		99.25329

				162.46		99.25329

				162.48		99.24731

				162.5		99.24731

				162.52		99.24731

				162.54		99.24731

				162.56		99.24731

				162.59		99.24134

				162.61		99.24134

				162.63		99.24134

				162.65		99.23536

				162.67		99.23536

				162.69		99.23536

				162.71		99.23536

				162.73		99.22939

				162.75		99.22939

				162.78		99.22939

				162.8		99.22939

				162.82		99.22939

				162.84		99.22342

				162.86		99.22342

				162.88		99.22342

				162.9		99.22342

				162.92		99.22342

				162.94		99.22342

				162.97		99.22342

				162.99		99.21744

				163.01		99.21744

				163.03		99.21744

				163.05		99.21744

				163.07		99.21147

				163.09		99.21147

				163.11		99.21147

				163.13		99.21147

				163.16		99.21147

				163.18		99.21147

				163.2		99.2055

				163.22		99.2055

				163.24		99.2055

				163.26		99.2055

				163.28		99.2055

				163.3		99.19952

				163.32		99.19952

				163.35		99.19355

				163.37		99.19355

				163.39		99.19355

				163.41		99.19355

				163.43		99.19355

				163.45		99.18757

				163.47		99.18757

				163.49		99.18757

				163.51		99.18757

				163.54		99.1816

				163.56		99.1816

				163.58		99.17563

				163.6		99.17563

				163.62		99.17563

				163.64		99.16965

				163.66		99.16965

				163.68		99.16965

				163.7		99.16368

				163.73		99.16368

				163.75		99.16368

				163.77		99.15771

				163.79		99.15771

				163.81		99.15771

				163.83		99.15173

				163.85		99.15173

				163.87		99.15173

				163.89		99.15173

				163.92		99.14576

				163.94		99.14576

				163.96		99.14576

				163.98		99.13978

				164		99.13381

				164.02		99.13978

				164.04		99.13381

				164.06		99.12784

				164.08		99.12784

				164.1		99.12784

				164.13		99.12784

				164.15		99.12186

				164.17		99.11589

				164.19		99.11589

				164.21		99.11589

				164.23		99.10992

				164.25		99.10992

				164.27		99.10394

				164.29		99.10394

				164.32		99.10394

				164.34		99.09797

				164.36		99.09797

				164.38		99.092

				164.4		99.092

				164.42		99.08602

				164.44		99.08602

				164.46		99.08602

				164.48		99.08005

				164.51		99.08005

				164.53		99.08005

				164.55		99.08005

				164.57		99.07407

				164.59		99.07407

				164.61		99.0681

				164.63		99.0681

				164.65		99.0681

				164.67		99.0681

				164.7		99.0681

				164.72		99.06213

				164.74		99.06213

				164.76		99.06213

				164.78		99.05615

				164.8		99.05018

				164.82		99.05018

				164.84		99.05018

				164.86		99.05018

				164.89		99.05018

				164.91		99.05018

				164.93		99.04421

				164.95		99.03823

				164.97		99.03823

				164.99		99.03823

				165.01		99.03226

				165.03		99.03823

				165.05		99.03823

				165.08		99.03226

				165.1		99.03226

				165.12		99.02628

				165.14		99.02628

				165.16		99.02031

				165.18		99.02031

				165.2		99.02031

				165.22		99.01434

				165.24		99.01434

				165.26		99.00836

				165.29		99.00836

				165.31		99.00239

				165.33		99.00239

				165.35		99.00239

				165.37		98.99642

				165.39		98.99642

				165.41		98.99642

				165.43		98.99642

				165.45		98.98447

				165.48		98.98447

				165.5		98.98447

				165.52		98.98447

				165.54		98.97849

				165.56		98.97849

				165.58		98.97849

				165.6		98.97849

				165.62		98.97252

				165.64		98.97252

				165.67		98.97252

				165.69		98.96655

				165.71		98.96655

				165.73		98.96655

				165.75		98.96057

				165.77		98.96057

				165.79		98.96057

				165.81		98.96057

				165.83		98.96057

				165.86		98.96057

				165.88		98.9546

				165.9		98.9546

				165.92		98.9546

				165.94		98.94863

				165.96		98.94863

				165.98		98.9546

				166		98.94863

				166.02		98.94863

				166.04		98.94265

				166.07		98.94265

				166.09		98.93668

				166.11		98.93668

				166.13		98.9307

				166.15		98.9307

				166.17		98.9307

				166.19		98.9307

				166.21		98.92473

				166.23		98.92473

				166.26		98.91876

				166.28		98.91876

				166.3		98.91278

				166.32		98.91278

				166.34		98.91278

				166.36		98.91278

				166.38		98.90681

				166.4		98.90681

				166.42		98.90084

				166.45		98.90084

				166.47		98.89486

				166.49		98.89486

				166.51		98.88889

				166.53		98.88889

				166.55		98.88292

				166.57		98.87694

				166.59		98.87694

				166.61		98.87694

				166.63		98.87097

				166.66		98.87097

				166.68		98.87097

				166.7		98.86499

				166.72		98.86499

				166.74		98.86499

				166.76		98.85902

				166.78		98.85902

				166.8		98.85902

				166.82		98.85902

				166.85		98.85902

				166.87		98.85305

				166.89		98.85305

				166.91		98.85305

				166.93		98.84707

				166.95		98.84707

				166.97		98.8411

				166.99		98.8411

				167.01		98.8411

				167.04		98.83513

				167.06		98.83513

				167.08		98.83513

				167.1		98.82915

				167.12		98.82915

				167.14		98.82915

				167.16		98.82318

				167.18		98.82318

				167.2		98.82318

				167.23		98.82318

				167.25		98.82318

				167.27		98.82318

				167.29		98.8172

				167.31		98.8172

				167.33		98.8172

				167.35		98.81123

				167.37		98.81123

				167.39		98.81123

				167.41		98.80526

				167.44		98.80526

				167.46		98.79928

				167.48		98.79928

				167.5		98.79928

				167.52		98.79331

				167.54		98.79331

				167.56		98.78734

				167.58		98.78734

				167.6		98.78136

				167.63		98.78734

				167.65		98.78136

				167.67		98.78136

				167.69		98.78136

				167.71		98.78136

				167.73		98.77539

				167.75		98.77539

				167.77		98.77539

				167.79		98.77539

				167.81		98.76941

				167.84		98.76941

				167.86		98.76941

				167.88		98.76344

				167.9		98.76344

				167.92		98.75747

				167.94		98.75747

				167.96		98.75149

				167.98		98.75149

				168		98.75149

				168.03		98.75149

				168.05		98.74552

				168.07		98.74552

				168.09		98.74552

				168.11		98.74552

				168.13		98.74552

				168.15		98.73955

				168.17		98.73357

				168.19		98.73357

				168.21		98.7276

				168.24		98.72162

				168.26		98.72162

				168.28		98.72162

				168.3		98.71565

				168.32		98.71565

				168.34		98.70968

				168.36		98.70968

				168.38		98.69773

				168.4		98.69773

				168.43		98.69176

				168.45		98.69176

				168.47		98.68578

				168.49		98.68578

				168.51		98.67981

				168.53		98.67981

				168.55		98.67981

				168.57		98.67981

				168.59		98.67384

				168.61		98.67384

				168.64		98.66786

				168.66		98.66786

				168.68		98.66189

				168.7		98.66189

				168.72		98.65591

				168.74		98.65591

				168.76		98.65591

				168.78		98.65591

				168.8		98.64994

				168.83		98.64994

				168.85		98.64994

				168.87		98.64397

				168.89		98.64397

				168.91		98.64397

				168.93		98.63799

				168.95		98.63799

				168.97		98.63799

				168.99		98.63799

				169.01		98.63202

				169.04		98.63202

				169.06		98.62605

				169.08		98.62605

				169.1		98.62007

				169.12		98.62007

				169.14		98.6141

				169.16		98.6141

				169.18		98.60812

				169.2		98.60812

				169.23		98.60215

				169.25		98.60215

				169.27		98.59618

				169.29		98.59618

				169.31		98.5902

				169.33		98.58423

				169.35		98.58423

				169.37		98.58423

				169.39		98.58423

				169.42		98.57826

				169.44		98.57228

				169.46		98.57228

				169.48		98.56631

				169.5		98.56631

				169.52		98.56033

				169.54		98.56033

				169.56		98.55436

				169.58		98.55436

				169.6		98.55436

				169.63		98.55436

				169.65		98.54839

				169.67		98.54839

				169.69		98.54241

				169.71		98.54241

				169.73		98.53644

				169.75		98.53644

				169.77		98.53047

				169.79		98.53047

				169.81		98.52449

				169.84		98.52449

				169.86		98.51852

				169.88		98.51852

				169.9		98.51254

				169.92		98.51254

				169.94		98.51254

				169.96		98.50657

				169.98		98.50657

				170		98.50657

				170.03		98.50657

				170.05		98.5006

				170.07		98.5006

				170.09		98.49462

				170.11		98.49462

				170.13		98.49462

				170.15		98.48865

				170.17		98.48865

				170.19		98.48865

				170.21		98.48268

				170.24		98.48268

				170.26		98.4767

				170.28		98.4767

				170.3		98.47073

				170.32		98.47073

				170.34		98.47073

				170.36		98.47073

				170.38		98.46476

				170.4		98.46476

				170.43		98.46476

				170.45		98.45878

				170.47		98.45878

				170.49		98.45878

				170.51		98.45281

				170.53		98.45281

				170.55		98.45281

				170.57		98.44683

				170.59		98.44683

				170.61		98.44086

				170.64		98.44086

				170.66		98.43489

				170.68		98.43489

				170.7		98.42891

				170.72		98.42891

				170.74		98.42891

				170.76		98.42294

				170.78		98.42294

				170.8		98.41697

				170.82		98.41099

				170.85		98.41099

				170.87		98.40502

				170.89		98.40502

				170.91		98.40502

				170.93		98.40502

				170.95		98.40502

				170.97		98.39904

				170.99		98.39307

				171.01		98.39307

				171.04		98.39307

				171.06		98.3871

				171.08		98.3871

				171.1		98.38112

				171.12		98.38112

				171.14		98.37515

				171.16		98.36918

				171.18		98.36918

				171.2		98.3632

				171.22		98.3632

				171.25		98.3632

				171.27		98.3632

				171.29		98.35723

				171.31		98.35723

				171.33		98.35723

				171.35		98.35125

				171.37		98.35125

				171.39		98.34528

				171.41		98.34528

				171.43		98.34528

				171.46		98.33931

				171.48		98.33931

				171.5		98.33333

				171.52		98.33333

				171.54		98.33333

				171.56		98.32736

				171.58		98.32139

				171.6		98.32139

				171.62		98.31541

				171.64		98.31541

				171.67		98.31541

				171.69		98.30944

				171.71		98.30944

				171.73		98.30944

				171.75		98.30346

				171.77		98.30346

				171.79		98.29749

				171.81		98.29749

				171.83		98.29152

				171.86		98.29152

				171.88		98.28554

				171.9		98.28554

				171.92		98.28554

				171.94		98.27957

				171.96		98.2736

				171.98		98.26762

				172		98.26762

				172.02		98.26165

				172.04		98.25568

				172.07		98.25568

				172.09		98.2497

				172.11		98.2497

				172.13		98.24373

				172.15		98.24373

				172.17		98.23775

				172.19		98.23775

				172.21		98.23178

				172.23		98.22581

				172.25		98.22581

				172.28		98.22581

				172.3		98.21983

				172.32		98.21386

				172.34		98.21386

				172.36		98.20789

				172.38		98.20191

				172.4		98.19594

				172.42		98.19594

				172.44		98.18996

				172.46		98.18399

				172.49		98.18399

				172.51		98.17802

				172.53		98.17802

				172.55		98.17204

				172.57		98.17204

				172.59		98.16607

				172.61		98.16607

				172.63		98.16607

				172.65		98.16607

				172.67		98.1601

				172.7		98.1601

				172.72		98.15412

				172.74		98.14815

				172.76		98.14815

				172.78		98.14217

				172.8		98.14815

				172.82		98.14217

				172.84		98.1362

				172.86		98.1362

				172.88		98.1362

				172.91		98.1362

				172.93		98.13023

				172.95		98.13023

				172.97		98.13023

				172.99		98.13023

				173.01		98.12425

				173.03		98.11828

				173.05		98.11231

				173.07		98.10633

				173.1		98.10633

				173.12		98.10633

				173.14		98.10036

				173.16		98.09438

				173.18		98.09438

				173.2		98.08841

				173.22		98.08244

				173.24		98.08244

				173.26		98.07646

				173.28		98.07646

				173.31		98.07646

				173.33		98.07049

				173.35		98.07049

				173.37		98.06452

				173.39		98.06452

				173.41		98.05854

				173.43		98.05257

				173.45		98.05257

				173.47		98.05257

				173.49		98.04659

				173.52		98.04659

				173.54		98.04659

				173.56		98.04062

				173.58		98.04062

				173.6		98.04062

				173.62		98.03465

				173.64		98.03465

				173.66		98.03465

				173.68		98.02867

				173.7		98.02867

				173.73		98.02867

				173.75		98.01673

				173.77		98.01673

				173.79		98.01075

				173.81		98.01075

				173.83		98.00478

				173.85		98.00478

				173.87		97.99881

				173.89		97.99881

				173.91		97.99881

				173.94		97.99283

				173.96		97.99283

				173.98		97.98686

				174		97.98088

				174.02		97.98686

				174.04		97.97491

				174.06		97.97491

				174.08		97.97491

				174.1		97.96894

				174.12		97.96894

				174.15		97.96296

				174.17		97.96296

				174.19		97.96894

				174.21		97.96296

				174.23		97.95699

				174.25		97.95699

				174.27		97.94504

				174.29		97.93907

				174.31		97.93907

				174.33		97.93907

				174.36		97.93309

				174.38		97.92712

				174.4		97.92115

				174.42		97.91517

				174.44		97.91517

				174.46		97.90323

				174.48		97.89725

				174.5		97.89128

				174.52		97.8853

				174.54		97.87336

				174.57		97.87336

				174.59		97.86738

				174.61		97.86738

				174.63		97.86141

				174.65		97.85544

				174.67		97.84946

				174.69		97.84349

				174.71		97.83751

				174.73		97.83154

				174.75		97.82557

				174.77		97.82557

				174.8		97.81959

				174.82		97.81362

				174.84		97.80765

				174.86		97.80765

				174.88		97.80167

				174.9		97.7957

				174.92		97.7957

				174.94		97.78973

				174.96		97.78973

				174.98		97.78375

				175.01		97.77778

				175.03		97.77778

				175.05		97.77778

				175.07		97.7718

				175.09		97.76583

				175.11		97.7718

				175.13		97.76583

				175.15		97.76583

				175.17		97.76583

				175.19		97.75986

				175.22		97.75388

				175.24		97.75388

				175.26		97.75986

				175.28		97.75388

				175.3		97.75388

				175.32		97.74791

				175.34		97.74791

				175.36		97.74194

				175.38		97.74194

				175.4		97.73596

				175.43		97.72999

				175.45		97.72999

				175.47		97.72999

				175.49		97.72401

				175.51		97.72401

				175.53		97.72401

				175.55		97.71804

				175.57		97.71207

				175.59		97.71207

				175.61		97.70609

				175.63		97.70012

				175.66		97.70012

				175.68		97.69415

				175.7		97.68817

				175.72		97.68817

				175.74		97.6822

				175.76		97.67622

				175.78		97.67025

				175.8		97.67025

				175.82		97.66428

				175.84		97.66428

				175.87		97.6583

				175.89		97.6583

				175.91		97.65233

				175.93		97.65233

				175.95		97.64636

				175.97		97.64038

				175.99		97.64038

				176.01		97.64038

				176.03		97.63441

				176.05		97.63441

				176.08		97.62843

				176.1		97.62843

				176.12		97.62843

				176.14		97.62246

				176.16		97.62246

				176.18		97.61649

				176.2		97.61649

				176.22		97.61051

				176.24		97.60454

				176.26		97.59857

				176.28		97.59857

				176.31		97.58662

				176.33		97.58662

				176.35		97.58065

				176.37		97.57467

				176.39		97.57467

				176.41		97.5687

				176.43		97.56272

				176.45		97.55675

				176.47		97.55078

				176.49		97.5448

				176.52		97.5448

				176.54		97.53883

				176.56		97.53286

				176.58		97.53286

				176.6		97.53286

				176.62		97.52688

				176.64		97.52688

				176.66		97.52091

				176.68		97.51493

				176.7		97.52091

				176.73		97.51493

				176.75		97.50896

				176.77		97.50299

				176.79		97.49701

				176.81		97.49701

				176.83		97.49104

				176.85		97.49104

				176.87		97.48507

				176.89		97.47909

				176.91		97.47312

				176.93		97.47312

				176.96		97.46714

				176.98		97.46117

				177		97.44922

				177.02		97.44325

				177.04		97.44325

				177.06		97.43728

				177.08		97.4313

				177.1		97.4313

				177.12		97.42533

				177.14		97.42533

				177.17		97.41935

				177.19		97.41935

				177.21		97.40741

				177.23		97.40741

				177.25		97.40143

				177.27		97.39546

				177.29		97.39546

				177.31		97.38949

				177.33		97.38351

				177.35		97.38949

				177.38		97.38351

				177.4		97.38351

				177.42		97.37754

				177.44		97.37754

				177.46		97.37157

				177.48		97.37157

				177.5		97.36559

				177.52		97.35962

				177.54		97.36559

				177.56		97.35962

				177.58		97.35364

				177.61		97.35364

				177.63		97.35364

				177.65		97.35364

				177.67		97.34767

				177.69		97.3417

				177.71		97.3417

				177.73		97.33572

				177.75		97.32975

				177.77		97.32975

				177.79		97.32378

				177.82		97.3178

				177.84		97.3178

				177.86		97.30585

				177.88		97.29988

				177.9		97.29988

				177.92		97.29391

				177.94		97.28196

				177.96		97.27599

				177.98		97.27599

				178		97.27599

				178.03		97.27001

				178.05		97.27001

				178.07		97.26404

				178.09		97.25806

				178.11		97.25806

				178.13		97.25209

				178.15		97.25209

				178.17		97.25209

				178.19		97.24612

				178.21		97.24014

				178.23		97.24014

				178.26		97.24014

				178.28		97.24014

				178.3		97.23417

				178.32		97.23417

				178.34		97.23417

				178.36		97.2282

				178.38		97.2282

				178.4		97.22222

				178.42		97.21625

				178.44		97.21027

				178.47		97.2043

				178.49		97.19833

				178.51		97.19833

				178.53		97.19235

				178.55		97.19235

				178.57		97.18638

				178.59		97.18041

				178.61		97.17443

				178.63		97.17443

				178.65		97.16846

				178.68		97.16249

				178.7		97.16249

				178.72		97.15651

				178.74		97.15054

				178.76		97.14456

				178.78		97.14456

				178.8		97.13859

				178.82		97.13262

				178.84		97.13262

				178.86		97.12664

				178.88		97.12067

				178.91		97.12067

				178.93		97.1147

				178.95		97.1147

				178.97		97.10872

				178.99		97.10872

				179.01		97.10275

				179.03		97.10275

				179.05		97.09677

				179.07		97.0908

				179.09		97.0908

				179.12		97.08483

				179.14		97.08483

				179.16		97.07885

				179.18		97.06691

				179.2		97.06691

				179.22		97.06691

				179.24		97.06691

				179.26		97.06093

				179.28		97.05496

				179.3		97.04898

				179.32		97.04301

				179.35		97.03704

				179.37		97.03106

				179.39		97.02509

				179.41		97.02509

				179.43		97.01314

				179.45		97.01314

				179.47		97.00717

				179.49		97.00717

				179.51		97.01314

				179.53		97.00717

				179.55		97.00119

				179.58		96.99522

				179.6		96.98925

				179.62		96.98925

				179.64		96.9773

				179.66		96.9773

				179.68		96.97133

				179.7		96.96535

				179.72		96.97133

				179.74		96.96535

				179.76		96.95341

				179.79		96.94743

				179.81		96.94146

				179.83		96.92951

				179.85		96.92354

				179.87		96.92354

				179.89		96.91756

				179.91		96.91756

				179.93		96.91756

				179.95		96.91159

				179.97		96.90562

				179.99		96.89964

				180.02		96.89964

				180.04		96.89964

				180.06		96.88769

				180.08		96.89367

				180.1		96.89367

				180.12		96.88769

				180.14		96.88769

				180.16		96.88172

				180.18		96.88172

				180.2		96.86977

				180.22		96.86977

				180.25		96.85783

				180.27		96.85185

				180.29		96.84588

				180.31		96.8399

				180.33		96.83393

				180.35		96.82796

				180.37		96.82198

				180.39		96.81601

				180.41		96.80406

				180.43		96.81004

				180.45		96.80406

				180.48		96.79809

				180.5		96.78614

				180.52		96.78614

				180.54		96.77419

				180.56		96.76822

				180.58		96.76822

				180.6		96.76225

				180.62		96.75627

				180.64		96.7503

				180.66		96.74432

				180.69		96.73835

				180.71		96.73238

				180.73		96.73238

				180.75		96.7264

				180.77		96.72043

				180.79		96.70848

				180.81		96.70848

				180.83		96.70251

				180.85		96.70251

				180.87		96.70848

				180.89		96.69654

				180.92		96.69654

				180.94		96.69654

				180.96		96.69056

				180.98		96.68459

				181		96.67861

				181.02		96.67861

				181.04		96.67861

				181.06		96.66667

				181.08		96.66667

				181.1		96.66069

				181.13		96.66069

				181.15		96.65472

				181.17		96.64875

				181.19		96.64277

				181.21		96.6368

				181.23		96.63082

				181.25		96.63082

				181.27		96.61888

				181.29		96.6129

				181.31		96.60693

				181.33		96.60693

				181.36		96.59498

				181.38		96.60096

				181.4		96.58901

				181.42		96.58901

				181.44		96.58303

				181.46		96.57706

				181.48		96.57109

				181.5		96.56511

				181.52		96.56511

				181.54		96.56511

				181.56		96.55317

				181.59		96.55317

				181.61		96.55317

				181.63		96.54719

				181.65		96.53524

				181.67		96.53524

				181.69		96.52927

				181.71		96.5233

				181.73		96.5233

				181.75		96.51732

				181.77		96.51732

				181.79		96.51135

				181.82		96.51135

				181.84		96.50538

				181.86		96.4994

				181.88		96.49343

				181.9		96.49343

				181.92		96.48746

				181.94		96.48148

				181.96		96.48746

				181.98		96.48148

				182		96.46953

				182.02		96.46953

				182.05		96.46356

				182.07		96.45759

				182.09		96.45759

				182.11		96.45161

				182.13		96.44564

				182.15		96.43967

				182.17		96.42772

				182.19		96.42772

				182.21		96.42174

				182.23		96.41577

				182.26		96.4098

				182.28		96.40382

				182.3		96.39785

				182.32		96.39188

				182.34		96.37993

				182.36		96.37395

				182.38		96.37395

				182.4		96.36201

				182.42		96.35603

				182.44		96.35603

				182.46		96.35006

				182.49		96.35006

				182.51		96.34409

				182.53		96.33811

				182.55		96.33214

				182.57		96.33214

				182.59		96.32616

				182.61		96.32019

				182.63		96.31422

				182.65		96.31422

				182.67		96.30824

				182.7		96.30227

				182.72		96.30227

				182.74		96.2963

				182.76		96.28435

				182.78		96.27838

				182.8		96.27838

				182.82		96.2724

				182.84		96.26045

				182.86		96.25448

				182.88		96.25448

				182.9		96.24851

				182.93		96.24253

				182.95		96.24253

				182.97		96.23059

				182.99		96.22461

				183.01		96.22461

				183.03		96.22461

				183.05		96.21864

				183.07		96.20669

				183.09		96.20669

				183.11		96.20072

				183.13		96.20072

				183.16		96.18877

				183.18		96.1828

				183.2		96.17682

				183.22		96.17682

				183.24		96.17085

				183.26		96.16487

				183.28		96.16487

				183.3		96.15293

				183.32		96.14695

				183.34		96.14098

				183.37		96.14098

				183.39		96.14098

				183.41		96.12306

				183.43		96.12903

				183.45		96.12306

				183.47		96.11708

				183.49		96.11111

				183.51		96.10514

				183.53		96.09916

				183.55		96.08722

				183.57		96.08722

				183.6		96.08124

				183.62		96.07527

				183.64		96.0693

				183.66		96.0693

				183.68		96.06332

				183.7		96.0454

				183.72		96.0454

				183.74		96.03943

				183.76		96.03345

				183.78		96.03345

				183.81		96.02748

				183.83		96.02151

				183.85		96.01553

				183.87		96.00956

				183.89		95.99761

				183.91		95.99164

				183.93		95.97969

				183.95		95.98566

				183.97		95.97969

				183.99		95.96774

				184.01		95.96774

				184.04		95.96177

				184.06		95.94982

				184.08		95.94982

				184.1		95.94982

				184.12		95.94385

				184.14		95.93787

				184.16		95.93787

				184.18		95.93787

				184.2		95.92593

				184.22		95.91995

				184.24		95.91398

				184.27		95.91398

				184.29		95.908

				184.31		95.908

				184.33		95.89606

				184.35		95.89008

				184.37		95.89008

				184.39		95.87814

				184.41		95.86619

				184.43		95.86619

				184.45		95.86619

				184.48		95.86022

				184.5		95.86022

				184.52		95.86022

				184.54		95.85424

				184.56		95.84827

				184.58		95.84229

				184.6		95.84229

				184.62		95.83632

				184.64		95.82437

				184.66		95.8184

				184.68		95.81243

				184.71		95.80048

				184.73		95.80048

				184.75		95.7945

				184.77		95.78853

				184.79		95.78256

				184.81		95.77061

				184.83		95.77061

				184.85		95.76464

				184.87		95.75866

				184.89		95.75269

				184.91		95.75269

				184.94		95.74074

				184.96		95.74074

				184.98		95.73477

				185		95.73477

				185.02		95.72879

				185.04		95.72282

				185.06		95.72282

				185.08		95.71685

				185.1		95.71087

				185.12		95.71685

				185.15		95.71087

				185.17		95.71087

				185.19		95.7049

				185.21		95.7049

				185.23		95.69892

				185.25		95.69295

				185.27		95.68698

				185.29		95.681

				185.31		95.66906

				185.33		95.66308

				185.35		95.65711

				185.38		95.66308

				185.4		95.64516

				185.42		95.63919

				185.44		95.63919

				185.46		95.63321

				185.48		95.62127

				185.5		95.62127

				185.52		95.62127

				185.54		95.61529

				185.56		95.60932

				185.58		95.61529

				185.61		95.60335

				185.63		95.5914

				185.65		95.58542

				185.67		95.58542

				185.69		95.57945

				185.71		95.5675

				185.73		95.56153

				185.75		95.56153

				185.77		95.54958

				185.79		95.54958

				185.82		95.53763

				185.84		95.53166

				185.86		95.52569

				185.88		95.51971

				185.9		95.51374

				185.92		95.50777

				185.94		95.50179

				185.96		95.49582

				185.98		95.48984

				186		95.48387

				186.02		95.4779

				186.05		95.4779

				186.07		95.46595

				186.09		95.46595

				186.11		95.45998

				186.13		95.45998

				186.15		95.44803

				186.17		95.44205

				186.19		95.43608

				186.21		95.43608

				186.23		95.42413

				186.25		95.41816

				186.28		95.40621

				186.3		95.40024

				186.32		95.39427

				186.34		95.38232

				186.36		95.37634

				186.38		95.37037

				186.4		95.3644

				186.42		95.3644

				186.44		95.35245

				186.46		95.35842

				186.48		95.34648

				186.51		95.35245

				186.53		95.34648

				186.55		95.33453

				186.57		95.33453

				186.59		95.33453

				186.61		95.31661

				186.63		95.31063

				186.65		95.30466

				186.67		95.29271

				186.69		95.28674

				186.71		95.27479

				186.74		95.27479

				186.76		95.26284

				186.78		95.25687

				186.8		95.2509

				186.82		95.23895

				186.84		95.24492

				186.86		95.23297

				186.88		95.23297

				186.9		95.23297

				186.92		95.23297

				186.94		95.22103

				186.97		95.22103

				186.99		95.20908

				187.01		95.21505

				187.03		95.20908

				187.05		95.20311

				187.07		95.20908

				187.09		95.19713

				187.11		95.19116

				187.13		95.17324

				187.15		95.17324

				187.17		95.16726

				187.2		95.15532

				187.22		95.15532

				187.24		95.14337

				187.26		95.13142

				187.28		95.12545

				187.3		95.10753

				187.32		95.1135

				187.34		95.10753

				187.36		95.10155

				187.38		95.09558

				187.41		95.08363

				187.43		95.08961

				187.45		95.07168

				187.47		95.06571

				187.49		95.05974

				187.51		95.05974

				187.53		95.04182

				187.55		95.02987

				187.57		95.02389

				187.59		95.01792

				187.61		95.00597

				187.64		95.00597

				187.66		95.01195

				187.68		94.99403

				187.7		95

				187.72		94.98805

				187.74		94.98805

				187.76		94.97611

				187.78		94.97611

				187.8		94.97013

				187.82		94.96416

				187.84		94.96416

				187.87		94.95818

				187.89		94.95221

				187.91		94.94624

				187.93		94.93429

				187.95		94.92832

				187.97		94.91637

				187.99		94.92234

				188.01		94.91039

				188.03		94.91039

				188.05		94.89845

				188.07		94.90442

				188.1		94.89247

				188.12		94.8865

				188.14		94.8865

				188.16		94.87455

				188.18		94.86858

				188.2		94.86858

				188.22		94.8626

				188.24		94.86858

				188.26		94.85066

				188.28		94.84468

				188.3		94.83871

				188.33		94.83871

				188.35		94.82676

				188.37		94.82676

				188.39		94.82079

				188.41		94.81481

				188.43		94.80884

				188.45		94.80287

				188.47		94.79689

				188.49		94.79092

				188.51		94.79092

				188.53		94.79092

				188.56		94.78495

				188.58		94.773

				188.6		94.773

				188.62		94.76105

				188.64		94.7491

				188.66		94.74313

				188.68		94.74313

				188.7		94.73118

				188.72		94.72521

				188.74		94.72521

				188.77		94.71326

				188.79		94.70729

				188.81		94.70131

				188.83		94.69534

				188.85		94.68339

				188.87		94.67742

				188.89		94.67145

				188.91		94.6595

				188.93		94.66547

				188.95		94.65352

				188.97		94.64158

				189		94.6356

				189.02		94.62963

				189.04		94.62366

				189.06		94.61768

				189.08		94.61768

				189.1		94.61768

				189.12		94.60573

				189.14		94.59976

				189.16		94.58781

				189.18		94.58781

				189.2		94.58184

				189.23		94.56989

				189.25		94.56392

				189.27		94.55197

				189.29		94.55197

				189.31		94.54002

				189.33		94.53405

				189.35		94.52808

				189.37		94.52808

				189.39		94.5221

				189.41		94.51016

				189.43		94.50418

				189.45		94.51016

				189.48		94.49821

				189.5		94.48029

				189.52		94.48626

				189.54		94.47431

				189.56		94.46834

				189.58		94.46834

				189.6		94.45639

				189.62		94.45042

				189.64		94.45042

				189.66		94.45042

				189.68		94.43847

				189.71		94.4325

				189.73		94.4325

				189.75		94.41458

				189.77		94.41458

				189.79		94.4086

				189.81		94.39665

				189.83		94.38471

				189.85		94.37276

				189.87		94.36679

				189.89		94.35484

				189.92		94.34886

				189.94		94.34289

				189.96		94.33692

				189.98		94.33094

				190		94.319

				190.02		94.31302

				190.04		94.31302

				190.06		94.30705

				190.08		94.30108

				190.1		94.28913

				190.12		94.28315

				190.15		94.27121

				190.17		94.26523

				190.19		94.25926

				190.21		94.25329

				190.23		94.25926

				190.25		94.24731

				190.27		94.23536

				190.29		94.22342

				190.31		94.22342

				190.33		94.21147

				190.35		94.21147

				190.38		94.2055

				190.4		94.19355

				190.42		94.1816

				190.44		94.16368

				190.46		94.16368

				190.48		94.15173

				190.5		94.14576

				190.52		94.14576

				190.54		94.13381

				190.56		94.13381

				190.58		94.11589

				190.6		94.10992

				190.63		94.10394

				190.65		94.09797

				190.67		94.10394

				190.69		94.092

				190.71		94.08602

				190.73		94.08602

				190.75		94.07407

				190.77		94.06213

				190.79		94.05615

				190.81		94.05615

				190.83		94.04421

				190.86		94.03823

				190.88		94.03823

				190.9		94.03226

				190.92		94.02031

				190.94		94.00836

				190.96		94.00836

				190.98		93.99642

				191		93.99642

				191.02		94.00239

				191.04		93.99642

				191.06		93.99044

				191.09		93.98447

				191.11		93.97252

				191.13		93.96655

				191.15		93.96655

				191.17		93.96057

				191.19		93.94265

				191.21		93.93668

				191.23		93.9307

				191.25		93.91278

				191.27		93.90681

				191.29		93.88889

				191.32		93.87694

				191.34		93.87694

				191.36		93.85902

				191.38		93.85305

				191.4		93.84707

				191.42		93.84707

				191.44		93.8411

				191.46		93.83513

				191.48		93.83513

				191.5		93.83513

				191.52		93.83513

				191.55		93.82915

				191.57		93.82915

				191.59		93.8172

				191.61		93.80526

				191.63		93.79928

				191.65		93.78734

				191.67		93.76941

				191.69		93.76344

				191.71		93.75149

				191.73		93.73357

				191.75		93.7276

				191.77		93.72162

				191.8		93.72162

				191.82		93.70968

				191.84		93.7037

				191.86		93.7037

				191.88		93.69176

				191.9		93.68578

				191.92		93.67981

				191.94		93.66786

				191.96		93.66189

				191.98		93.66189

				192		93.64994

				192.03		93.63799

				192.05		93.63799

				192.07		93.62605

				192.09		93.62605

				192.11		93.62007

				192.13		93.6141

				192.15		93.60812

				192.17		93.60812

				192.19		93.5902

				192.21		93.57826

				192.23		93.57826

				192.25		93.56631

				192.28		93.54839

				192.3		93.54839

				192.32		93.54241

				192.34		93.52449

				192.36		93.51852

				192.38		93.51852

				192.4		93.51254

				192.42		93.50657

				192.44		93.50657

				192.46		93.50657

				192.48		93.5006

				192.51		93.48865

				192.53		93.48268

				192.55		93.47073

				192.57		93.47073

				192.59		93.47073

				192.61		93.45878

				192.63		93.45281

				192.65		93.44683

				192.67		93.44086

				192.69		93.42891

				192.71		93.41697

				192.74		93.42294

				192.76		93.40502

				192.78		93.39307

				192.8		93.39307

				192.82		93.37515

				192.84		93.36918

				192.86		93.35723

				192.88		93.35723

				192.9		93.35723

				192.92		93.35723

				192.94		93.34528

				192.97		93.34528

				192.99		93.35723

				193.01		93.33931

				193.03		93.33333

				193.05		93.33333

				193.07		93.32139

				193.09		93.30346

				193.11		93.29749

				193.13		93.28554

				193.15		93.27957

				193.17		93.26165

				193.2		93.25568

				193.22		93.23775

				193.24		93.22581

				193.26		93.22581

				193.28		93.21983

				193.3		93.20789

				193.32		93.20789

				193.34		93.19594

				193.36		93.18996

				193.38		93.17204

				193.4		93.17204

				193.43		93.16607

				193.45		93.15412

				193.47		93.15412

				193.49		93.1601

				193.51		93.14815

				193.53		93.14815

				193.55		93.14217

				193.57		93.15412

				193.59		93.14217

				193.61		93.13023

				193.63		93.11828

				193.66		93.10036

				193.68		93.08841

				193.7		93.07646

				193.72		93.05854

				193.74		93.05257

				193.76		93.03465

				193.78		93.0227

				193.8		93.01673

				193.82		93.01673

				193.84		93.01075

				193.86		93.00478

				193.89		92.99881

				193.91		92.99881

				193.93		92.98686

				193.95		92.98088

				193.97		92.98088

				193.99		92.98088

				194.01		92.96894

				194.03		92.96296

				194.05		92.95102

				194.07		92.93907

				194.09		92.92712

				194.12		92.93309

				194.14		92.92115

				194.16		92.91517

				194.18		92.90323

				194.2		92.89725

				194.22		92.8853

				194.24		92.87933

				194.26		92.87336

				194.28		92.86738

				194.3		92.84946

				194.32		92.84349

				194.35		92.83154

				194.37		92.82557

				194.39		92.81959

				194.41		92.81362

				194.43		92.80167

				194.45		92.78973

				194.47		92.78375

				194.49		92.77778

				194.51		92.76583

				194.53		92.75388

				194.55		92.74791

				194.58		92.73596

				194.6		92.72999

				194.62		92.72401

				194.64		92.72999

				194.66		92.70609

				194.68		92.70012

				194.7		92.68817

				194.72		92.6822

				194.74		92.66428

				194.76		92.66428

				194.78		92.64636

				194.81		92.63441

				194.83		92.62246

				194.85		92.62246

				194.87		92.61649

				194.89		92.61051

				194.91		92.61051

				194.93		92.61051

				194.95		92.59259

				194.97		92.59857

				194.99		92.58662

				195.01		92.5687

				195.04		92.56272

				195.06		92.5448

				195.08		92.55078

				195.1		92.52688

				195.12		92.51493

				195.14		92.51493

				195.16		92.50896

				195.18		92.50299

				195.2		92.50299

				195.22		92.49701

				195.24		92.49701

				195.26		92.48507

				195.29		92.47909

				195.31		92.47909

				195.33		92.47312

				195.35		92.46117

				195.37		92.44922

				195.39		92.4313

				195.41		92.4313

				195.43		92.41338

				195.45		92.40741

				195.47		92.39546

				195.49		92.38351

				195.52		92.37157

				195.54		92.35962

				195.56		92.35962

				195.58		92.35364

				195.6		92.3417

				195.62		92.32975

				195.64		92.32378

				195.66		92.31183

				195.68		92.30585

				195.7		92.30585

				195.72		92.29391

				195.75		92.28793

				195.77		92.27599

				195.79		92.27001

				195.81		92.27001

				195.83		92.24612

				195.85		92.24612

				195.87		92.2282

				195.89		92.22222

				195.91		92.21027

				195.93		92.2043

				195.95		92.19833

				195.98		92.18638

				196		92.16846

				196.02		92.16846

				196.04		92.16249

				196.06		92.15651

				196.08		92.14456

				196.1		92.13859

				196.12		92.12664

				196.14		92.13262

				196.16		92.13262

				196.18		92.12067

				196.21		92.10275

				196.23		92.10872

				196.25		92.09677

				196.27		92.08483

				196.29		92.07288

				196.31		92.05496

				196.33		92.04898

				196.35		92.03106

				196.37		92.01912

				196.39		92.01314

				196.41		92.00717

				196.44		91.99522

				196.46		92.00119

				196.48		91.98327

				196.5		91.9773

				196.52		91.96535

				196.54		91.95938

				196.56		91.94146

				196.58		91.92951

				196.6		91.91756

				196.62		91.90562

				196.64		91.89367

				196.67		91.87575

				196.69		91.85783

				196.71		91.85185

				196.73		91.83393

				196.75		91.82796

				196.77		91.82198

				196.79		91.81601

				196.81		91.80406

				196.83		91.80406

				196.85		91.80406

				196.87		91.80406

				196.9		91.78017

				196.92		91.78017

				196.94		91.77419

				196.96		91.76822

				196.98		91.75627

				197		91.74432

				197.02		91.73238

				197.04		91.73238

				197.06		91.71446

				197.08		91.69654

				197.1		91.69654

				197.13		91.68459

				197.15		91.68459

				197.17		91.67861

				197.19		91.66667

				197.21		91.66069

				197.23		91.65472

				197.25		91.64277

				197.27		91.63082

				197.29		91.62485

				197.31		91.6129

				197.33		91.60693

				197.36		91.60096

				197.38		91.58901

				197.4		91.58303

				197.42		91.57109

				197.44		91.56511

				197.46		91.55914

				197.48		91.55317

				197.5		91.54719

				197.52		91.52927

				197.54		91.52927

				197.56		91.51732

				197.59		91.51135

				197.61		91.49343

				197.63		91.48148

				197.65		91.47551

				197.67		91.46356

				197.69		91.45759

				197.71		91.45161

				197.73		91.43967

				197.75		91.43369

				197.77		91.41577

				197.79		91.40382

				197.82		91.3859

				197.84		91.3859

				197.86		91.3859

				197.88		91.37993

				197.9		91.37395

				197.92		91.36798

				197.94		91.35603

				197.96		91.35603

				197.98		91.34409

				198		91.33214

				198.02		91.30824

				198.05		91.30227

				198.07		91.30227

				198.09		91.30227

				198.11		91.28435

				198.13		91.28435

				198.15		91.2724

				198.17		91.26643

				198.19		91.25448

				198.21		91.23656

				198.23		91.21266

				198.25		91.21864

				198.28		91.19474

				198.3		91.18877

				198.32		91.17682

				198.34		91.17682

				198.36		91.17085

				198.38		91.16487

				198.4		91.15293

				198.42		91.15293

				198.44		91.14098

				198.46		91.12903

				198.48		91.11111

				198.51		91.10514

				198.53		91.09319

				198.55		91.07527

				198.57		91.06332

				198.59		91.05735

				198.61		91.05137

				198.63		91.05137

				198.65		91.03345

				198.67		91.03345

				198.69		91.02748

				198.71		91.01553

				198.74		90.99164

				198.76		90.98566

				198.78		90.97372

				198.8		90.96774

				198.82		90.95579

				198.84		90.94982

				198.86		90.93787

				198.88		90.94385

				198.9		90.93787

				198.92		90.92593

				198.94		90.92593

				198.97		90.91398

				198.99		90.908

				199.01		90.90203

				199.03		90.89008

				199.05		90.87814

				199.07		90.86619

				199.09		90.85424

				199.11		90.83632

				199.13		90.82437

				199.15		90.81243

				199.17		90.7945

				199.2		90.77658

				199.22		90.77061

				199.24		90.74671

				199.26		90.74671

				199.28		90.72879

				199.3		90.72282

				199.32		90.71685

				199.34		90.71685

				199.36		90.69892

				199.38		90.69295

				199.4		90.681

				199.43		90.69295

				199.45		90.67503

				199.47		90.66906

				199.49		90.65114

				199.51		90.64516

				199.53		90.63919

				199.55		90.62724

				199.57		90.59737

				199.59		90.5914

				199.61		90.58542

				199.63		90.57945

				199.65		90.56153

				199.68		90.54958

				199.7		90.54361

				199.72		90.53166

				199.74		90.50777

				199.76		90.50179

				199.78		90.48387

				199.8		90.4779

				199.82		90.46595

				199.84		90.44803

				199.86		90.44205

				199.88		90.44803

				199.91		90.43011

				199.93		90.43608

				199.95		90.42413

				199.97		90.42413

				199.99		90.43011

				200.01		90.42413

				200.03		90.41219

				200.05		90.40621

				200.07		90.38232

				200.09		90.37634

				200.11		90.34648

				200.14		90.32855

				200.16		90.30466

				200.18		90.29271

				200.2		90.28076

				200.22		90.26882

				200.24		90.25687

				200.26		90.26284

				200.28		90.24492

				200.3		90.24492

				200.32		90.227

				200.34		90.227

				200.37		90.20908

				200.39		90.20311

				200.41		90.18519

				200.43		90.17324

				200.45		90.14934

				200.47		90.14337

				200.49		90.12545

				200.51		90.12545

				200.53		90.1135

				200.55		90.10753

				200.57		90.08961

				200.6		90.08363

				200.62		90.07168

				200.64		90.05974

				200.66		90.04779

				200.68		90.03584

				200.7		90.03584

				200.72		90.02389

				200.74		90.01195

				200.76		90.00597

				200.78		89.98805

				200.8		89.97013

				200.83		89.96416

				200.85		89.93429

				200.87		89.92832

				200.89		89.92832

				200.91		89.91637

				200.93		89.91637

				200.95		89.91637

				200.97		89.90442

				200.99		89.89845

				201.01		89.8865

				201.03		89.87455

				201.06		89.85663

				201.08		89.84468

				201.1		89.82676

				201.12		89.81481

				201.14		89.80287

				201.16		89.78495

				201.18		89.773

				201.2		89.76105

				201.22		89.73716

				201.24		89.71924

				201.26		89.71326

				201.29		89.70729

				201.31		89.69534

				201.33		89.68339

				201.35		89.67742

				201.37		89.67145

				201.39		89.66547

				201.41		89.64755

				201.43		89.64158

				201.45		89.62366

				201.47		89.61768

				201.49		89.59976

				201.52		89.59976

				201.54		89.58781

				201.56		89.58184

				201.58		89.56392

				201.6		89.55795

				201.62		89.55197

				201.64		89.54002

				201.66		89.5221

				201.68		89.51016

				201.7		89.50418

				201.72		89.49223

				201.75		89.48029

				201.77		89.46237

				201.79		89.45639

				201.81		89.44444

				201.83		89.42652

				201.85		89.41458

				201.87		89.41458

				201.89		89.40263

				201.91		89.39068

				201.93		89.37873

				201.95		89.36679

				201.98		89.36081

				202		89.34289

				202.02		89.319

				202.04		89.30108

				202.06		89.2951

				202.08		89.28315

				202.1		89.27718

				202.12		89.26523

				202.14		89.25329

				202.16		89.25329

				202.18		89.22939

				202.21		89.22939

				202.23		89.21147

				202.25		89.19952

				202.27		89.17563

				202.29		89.16368

				202.31		89.15173

				202.33		89.15173

				202.35		89.11589

				202.37		89.10992

				202.39		89.09797

				202.41		89.092

				202.44		89.08005

				202.46		89.07407

				202.48		89.0681

				202.5		89.05018

				202.52		89.05018

				202.54		89.02628

				202.56		89.02031

				202.58		89.01434

				202.6		89.00239

				202.62		88.98447

				202.65		88.99044

				202.67		88.98447

				202.69		88.96655

				202.71		88.9546

				202.73		88.9307

				202.75		88.93668

				202.77		88.92473

				202.79		88.90084

				202.81		88.88889

				202.83		88.88292

				202.85		88.84707

				202.88		88.82915

				202.9		88.82318

				202.92		88.80526

				202.94		88.79331

				202.96		88.79928

				202.98		88.78734

				203		88.77539

				203.02		88.76941

				203.04		88.75747

				203.06		88.73955

				203.08		88.7276

				203.11		88.7037

				203.13		88.7037

				203.15		88.67981

				203.17		88.67384

				203.19		88.65591

				203.21		88.66786

				203.23		88.63799

				203.25		88.63799

				203.27		88.62007

				203.29		88.6141

				203.31		88.58423

				203.34		88.57826

				203.36		88.57228

				203.38		88.54839

				203.4		88.54241

				203.42		88.54241

				203.44		88.54839

				203.46		88.51852

				203.48		88.54241

				203.5		88.51254

				203.52		88.48865

				203.54		88.45878

				203.57		88.45281

				203.59		88.41697

				203.61		88.41099

				203.63		88.39904

				203.65		88.3871

				203.67		88.37515

				203.69		88.3632

				203.71		88.34528

				203.73		88.35125

				203.75		88.34528

				203.77		88.32139

				203.8		88.32736

				203.82		88.31541

				203.84		88.29749

				203.86		88.28554

				203.88		88.29152

				203.9		88.2736

				203.92		88.25568

				203.94		88.24373

				203.96		88.21386

				203.98		88.20789

				204		88.18399

				204.03		88.17802

				204.05		88.16607

				204.07		88.17204

				204.09		88.14217

				204.11		88.14217

				204.13		88.12425

				204.15		88.11231

				204.17		88.09438

				204.19		88.08841

				204.21		88.05854

				204.23		88.05854

				204.26		88.04062

				204.28		88.0227

				204.3		87.99881

				204.32		87.99283

				204.34		87.96894

				204.36		87.92712

				204.38		87.91517

				204.4		87.91517

				204.42		87.9092

				204.44		87.89725

				204.46		87.91517

				204.49		87.90323

				204.51		87.89128

				204.53		87.87933

				204.55		87.85544

				204.57		87.83154

				204.59		87.81362

				204.61		87.81362

				204.63		87.78375

				204.65		87.78375

				204.67		87.78973

				204.69		87.76583

				204.72		87.73596

				204.74		87.74194

				204.76		87.72401

				204.78		87.69415

				204.8		87.6822

				204.82		87.6822

				204.84		87.67025

				204.86		87.63441

				204.88		87.64038

				204.9		87.62843

				204.93		87.60454

				204.95		87.59857

				204.97		87.60454

				204.99		87.59857

				205.01		87.58065

				205.03		87.58065

				205.05		87.56272

				205.07		87.5448

				205.09		87.52091

				205.11		87.53286

				205.13		87.49701

				205.16		87.47312

				205.18		87.47312

				205.2		87.44922

				205.22		87.42533

				205.24		87.41338

				205.26		87.40143

				205.28		87.36559

				205.3		87.35962

				205.32		87.3417

				205.34		87.3417

				205.36		87.32975

				205.39		87.33572

				205.41		87.32975

				205.43		87.31183

				205.45		87.29391

				205.47		87.29988

				205.49		87.27599

				205.51		87.24014

				205.53		87.23417

				205.55		87.21027

				205.57		87.18638

				205.59		87.18041

				205.62		87.16846

				205.64		87.15054

				205.66		87.13859

				205.68		87.12664

				205.7		87.10275

				205.72		87.09677

				205.74		87.0908

				205.76		87.08483

				205.78		87.05496

				205.8		87.04898

				205.82		87.04898

				205.85		87.03106

				205.87		87.00717

				205.89		87.00717

				205.91		86.98925

				205.93		86.95938

				205.95		86.97133

				205.97		86.94743

				205.99		86.91756

				206.01		86.91159

				206.03		86.91756

				206.05		86.86977

				206.08		86.86977

				206.1		86.8638

				206.12		86.84588

				206.14		86.81004

				206.16		86.81004

				206.18		86.79809

				206.2		86.76822

				206.22		86.74432

				206.24		86.7503

				206.26		86.7264

				206.29		86.71446

				206.31		86.71446

				206.33		86.73238

				206.35		86.70251

				206.37		86.69056

				206.39		86.66667

				206.41		86.66667

				206.43		86.63082

				206.45		86.6368

				206.47		86.61888

				206.49		86.60693

				206.52		86.58303

				206.54		86.60096

				206.56		86.55914

				206.58		86.54122

				206.6		86.53524

				206.62		86.5233

				206.64		86.46356

				206.66		86.47551

				206.68		86.46953

				206.7		86.45161

				206.73		86.41577

				206.75		86.42772

				206.77		86.39785

				206.79		86.3859

				206.81		86.36201

				206.83		86.37395

				206.85		86.35006

				206.87		86.34409

				206.89		86.32019

				206.91		86.33214

				206.93		86.30227

				206.96		86.30227

				206.98		86.2724

				207		86.25448

				207.02		86.22461

				207.04		86.23059

				207.06		86.20072

				207.08		86.20072

				207.1		86.19474

				207.12		86.18877

				207.14		86.13501

				207.17		86.14098

				207.19		86.11111

				207.21		86.09916

				207.23		86.08722

				207.25		86.10514

				207.27		86.08124

				207.29		86.0693

				207.31		86.03943

				207.33		86.03943

				207.35		86.01553

				207.37		86.00956

				207.4		86.00358

				207.42		85.98566

				207.44		85.95579

				207.46		85.94982

				207.48		85.91398

				207.5		85.908

				207.52		85.89606

				207.54		85.87814

				207.56		85.86022

				207.58		85.85424

				207.61		85.82437

				207.63		85.80645

				207.65		85.7945

				207.67		85.77061

				207.69		85.75866

				207.71		85.73477

				207.73		85.71087

				207.75		85.7049

				207.77		85.69892

				207.79		85.67503

				207.81		85.67503

				207.84		85.66308

				207.86		85.65114

				207.88		85.63321

				207.9		85.61529

				207.92		85.60932

				207.94		85.60335

				207.96		85.5914

				207.98		85.56153

				208		85.54958

				208.02		85.51374

				208.05		85.49582

				208.07		85.47192

				208.09		85.46595

				208.11		85.44803

				208.13		85.454

				208.15		85.41219

				208.17		85.41219

				208.19		85.40024

				208.21		85.37634

				208.23		85.34648

				208.25		85.34648

				208.28		85.32855

				208.3		85.29869

				208.32		85.31063

				208.34		85.29271

				208.36		85.27479

				208.38		85.26882

				208.4		85.26882

				208.42		85.23297

				208.44		85.22103

				208.46		85.21505

				208.49		85.19116

				208.51		85.17324

				208.53		85.17324

				208.55		85.16726

				208.57		85.14934

				208.59		85.13142

				208.61		85.11947

				208.63		85.1135

				208.65		85.07766

				208.67		85.07168

				208.69		85.05376

				208.72		85.02987

				208.74		84.98208

				208.76		84.98208

				208.78		84.95818

				208.8		84.93429

				208.82		84.91637

				208.84		84.91039

				208.86		84.8865

				208.88		84.88053

				208.9		84.88053

				208.93		84.86858

				208.95		84.85066

				208.97		84.84468

				208.99		84.82079

				209.01		84.79092

				209.03		84.773

				209.05		84.76105

				209.07		84.7491

				209.09		84.7491

				209.11		84.73716

				209.14		84.72521

				209.16		84.70131

				209.18		84.67742

				209.2		84.65352

				209.22		84.64158

				209.24		84.59379

				209.26		84.59379

				209.28		84.56989

				209.3		84.55197

				209.32		84.53405

				209.34		84.546

				209.37		84.5221

				209.39		84.52808

				209.41		84.51016

				209.43		84.49821

				209.45		84.48029

				209.47		84.45639

				209.49		84.43847

				209.51		84.42652

				209.53		84.40263

				209.55		84.39068

				209.58		84.39068

				209.6		84.35484

				209.62		84.34289

				209.64		84.32497

				209.66		84.31302

				209.68		84.26523

				209.7		84.25329

				209.72		84.22939

				209.74		84.21147

				209.76		84.1816

				209.78		84.19355

				209.81		84.16965

				209.83		84.14576

				209.85		84.12784

				209.87		84.12186

				209.89		84.10394

				209.91		84.092

				209.93		84.08602

				209.95		84.06213

				209.97		84.05018

				209.99		84.02031

				210.01		84.01434

				210.04		83.99044

				210.06		83.99044

				210.08		83.96057

				210.1		83.94863

				210.12		83.92473

				210.14		83.91278

				210.16		83.88292

				210.18		83.86499

				210.2		83.85902

				210.22		83.8411

				210.25		83.81123

				210.27		83.79331

				210.29		83.79928

				210.31		83.76344

				210.33		83.74552

				210.35		83.73955

				210.37		83.73357

				210.39		83.68578

				210.41		83.69176

				210.43		83.67981

				210.45		83.64994

				210.48		83.62605

				210.5		83.63202

				210.52		83.60215

				210.54		83.58423

				210.56		83.57826

				210.58		83.56033

				210.6		83.52449

				210.62		83.50657

				210.64		83.48865

				210.66		83.44683

				210.69		83.42294

				210.71		83.43489

				210.73		83.39904

				210.75		83.37515

				210.77		83.36918

				210.79		83.36918

				210.81		83.33931

				210.83		83.33333

				210.85		83.33931

				210.87		83.32736

				210.89		83.27957

				210.92		83.27957

				210.94		83.26762

				210.96		83.23775

				210.98		83.22581

				211		83.2497

				211.02		83.20191

				211.04		83.17802

				211.06		83.17204

				211.08		83.15412

				211.1		83.11828

				211.13		83.12425

				211.15		83.10036

				211.17		83.07646

				211.19		83.04659

				211.21		83.04659

				211.23		83.01673

				211.25		82.99283

				211.27		82.98088

				211.29		82.97491

				211.31		82.93309

				211.33		82.93309

				211.36		82.93907

				211.38		82.92712

				211.4		82.8853

				211.42		82.89725

				211.44		82.87933

				211.46		82.84349

				211.48		82.80765

				211.5		82.81362

				211.52		82.75986

				211.54		82.74194

				211.57		82.72401

				211.59		82.72999

				211.61		82.6822

				211.63		82.67622

				211.65		82.65233

				211.67		82.63441

				211.69		82.58662

				211.71		82.59857

				211.73		82.57467

				211.75		82.57467

				211.78		82.5448

				211.8		82.55675

				211.82		82.51493

				211.84		82.52091

				211.86		82.50299

				211.88		82.49701

				211.9		82.47909

				211.92		82.48507

				211.94		82.4552

				211.96		82.41935

				211.99		82.40143

				212.01		82.40143

				212.03		82.35364

				212.05		82.33572

				212.07		82.32378

				212.09		82.31183

				212.11		82.27001

				212.13		82.28793

				212.15		82.26404

				212.17		82.24014

				212.19		82.22222

				212.22		82.21027

				212.24		82.16846

				212.26		82.15054

				212.28		82.13859

				212.3		82.1147

				212.32		82.08483

				212.34		82.07288

				212.36		82.07288

				212.38		82.05496

				212.4		82.01314

				212.43		82.01912

				212.45		82.00717

				212.47		81.97133

				212.49		81.96535

				212.51		81.9773

				212.53		81.94146

				212.55		81.92354

				212.57		81.89367

				212.59		81.85783

				212.61		81.81601

				212.64		81.81601

				212.66		81.79211

				212.68		81.78614

				212.7		81.77419

				212.72		81.77419

				212.74		81.74432

				212.76		81.72043

				212.78		81.70848

				212.8		81.69056

				212.82		81.6368

				212.85		81.64277

				212.87		81.64277

				212.89		81.60693

				212.91		81.59498

				212.93		81.61888

				212.95		81.55914

				212.97		81.52927

				212.99		81.51732

				213.01		81.4994

				213.03		81.46356

				213.05		81.47551

				213.08		81.45759

				213.1		81.43967

				213.12		81.40382

				213.14		81.40382

				213.16		81.36798

				213.18		81.35603

				213.2		81.34409

				213.22		81.33214

				213.24		81.27838

				213.26		81.26643

				213.29		81.24851

				213.31		81.21864

				213.33		81.19474

				213.35		81.19474

				213.37		81.17682

				213.39		81.17085

				213.41		81.15293

				213.43		81.14695

				213.45		81.11111

				213.47		81.08722

				213.5		81.03943

				213.52		81.03345

				213.54		80.97969

				213.56		80.97969

				213.58		80.96774

				213.6		80.95579

				213.62		80.9319

				213.64		80.92593

				213.66		80.88411

				213.68		80.85424

				213.7		80.84229

				213.73		80.81243

				213.75		80.78256

				213.77		80.78256

				213.79		80.77658

				213.81		80.75269

				213.83		80.73477

				213.85		80.72282

				213.87		80.71685

				213.89		80.681

				213.91		80.66308

				213.94		80.63919

				213.96		80.62724

				213.98		80.60335

				214		80.57348

				214.02		80.5675

				214.04		80.54958

				214.06		80.51971

				214.08		80.49582

				214.1		80.49582

				214.12		80.454

				214.15		80.44205

				214.17		80.41219

				214.19		80.39427

				214.21		80.37037

				214.23		80.3644

				214.25		80.35842

				214.27		80.33453

				214.29		80.32855

				214.31		80.30466

				214.33		80.28674

				214.36		80.25687

				214.38		80.25687

				214.4		80.21505

				214.42		80.19116

				214.44		80.16129

				214.46		80.13142

				214.48		80.10753

				214.5		80.10155

				214.52		80.07766

				214.54		80.04779

				214.56		80.03584

				214.59		80.00597

				214.61		79.98805

				214.63		79.95818

				214.65		79.95221

				214.67		79.93429

				214.69		79.91637

				214.71		79.90442

				214.73		79.89247

				214.75		79.85663

				214.77		79.85066

				214.8		79.83871

				214.82		79.79689

				214.84		79.79689

				214.86		79.77897

				214.88		79.75508

				214.9		79.73118

				214.92		79.71326

				214.94		79.67742

				214.96		79.6595

				214.98		79.62963

				215.01		79.61768

				215.03		79.59379

				215.05		79.57587

				215.07		79.55795

				215.09		79.54002

				215.11		79.49821

				215.13		79.48029

				215.15		79.45639

				215.17		79.42652

				215.19		79.40263

				215.22		79.39068

				215.24		79.36679

				215.26		79.34289

				215.28		79.33692

				215.3		79.31302

				215.32		79.28913

				215.34		79.27121

				215.36		79.26523

				215.38		79.22939

				215.4		79.21147

				215.43		79.1816

				215.45		79.16965

				215.47		79.13381

				215.49		79.11589

				215.51		79.10394

				215.53		79.092

				215.55		79.06213

				215.57		79.03823

				215.59		79.00239

				215.61		78.96057

				215.64		78.93668

				215.66		78.91876

				215.68		78.91278

				215.7		78.90681

				215.72		78.90681

				215.74		78.88292

				215.76		78.85902

				215.78		78.8172

				215.8		78.80526

				215.82		78.78136

				215.85		78.75747

				215.87		78.73357

				215.89		78.7276

				215.91		78.69773

				215.93		78.67981

				215.95		78.65591

				215.97		78.64397

				215.99		78.62007

				216.01		78.5902

				216.03		78.56631

				216.06		78.56033

				216.08		78.52449

				216.1		78.51254

				216.12		78.48865

				216.14		78.45878

				216.16		78.42891

				216.18		78.41099

				216.2		78.3632

				216.22		78.3632

				216.24		78.32736

				216.27		78.30346

				216.29		78.2736

				216.31		78.2497

				216.33		78.21983

				216.35		78.21386

				216.37		78.20191

				216.39		78.18399

				216.41		78.17204

				216.43		78.15412

				216.45		78.13023

				216.47		78.11231

				216.5		78.08841

				216.52		78.07049

				216.54		78.0227

				216.56		78.00478

				216.58		77.97491

				216.6		77.93907

				216.62		77.9092

				216.64		77.9092

				216.66		77.8853

				216.68		77.86141

				216.71		77.84349

				216.73		77.83154

				216.75		77.80167

				216.77		77.76583

				216.79		77.75388

				216.81		77.73596

				216.83		77.71207

				216.85		77.6822

				216.87		77.6822

				216.89		77.66428

				216.92		77.62843

				216.94		77.61649

				216.96		77.60454

				216.98		77.5687

				217		77.53883

				217.02		77.53883

				217.04		77.49104

				217.06		77.47312

				217.08		77.44922

				217.1		77.41935

				217.13		77.38351

				217.15		77.35962

				217.17		77.3417

				217.19		77.31183

				217.21		77.29988

				217.23		77.28793

				217.25		77.27599

				217.27		77.23417

				217.29		77.21625

				217.31		77.2043

				217.34		77.16846

				217.36		77.13262

				217.38		77.13262

				217.4		77.10275

				217.42		77.07288

				217.44		77.06691

				217.46		77.07288

				217.48		77.03106

				217.5		77.01912

				217.52		77.00119

				217.55		76.95341

				217.57		76.90562

				217.59		76.88769

				217.61		76.87575

				217.63		76.84588

				217.65		76.83393

				217.67		76.82796

				217.69		76.81004

				217.71		76.76225

				217.73		76.7503

				217.76		76.71446

				217.78		76.67861

				217.8		76.65472

				217.82		76.64277

				217.84		76.6129

				217.86		76.59498

				217.88		76.58303

				217.9		76.54719

				217.92		76.51732

				217.94		76.51732

				217.97		76.48148

				217.99		76.45161

				218.01		76.43369

				218.03		76.42174

				218.05		76.35603

				218.07		76.35006

				218.09		76.33214

				218.11		76.30227

				218.13		76.25448

				218.15		76.25448

				218.18		76.21266

				218.2		76.17682

				218.22		76.16487

				218.24		76.14695

				218.26		76.11708

				218.28		76.09916

				218.3		76.09916

				218.32		76.07527

				218.34		76.05137

				218.36		76.0454

				218.39		76.02151

				218.41		75.98566

				218.43		75.96177

				218.45		75.94982

				218.47		75.908

				218.49		75.88411

				218.51		75.86619

				218.53		75.84229

				218.55		75.7945

				218.57		75.77061

				218.6		75.74671

				218.62		75.71087

				218.64		75.68698

				218.66		75.681

				218.68		75.65711

				218.7		75.64516

				218.72		75.62127

				218.74		75.60335

				218.76		75.57348

				218.78		75.55556

				218.81		75.51374

				218.83		75.48984

				218.85		75.44803

				218.87		75.44205

				218.89		75.40024

				218.91		75.37634

				218.93		75.35245

				218.95		75.33453

				218.97		75.28674

				218.99		75.26882

				219.02		75.25687

				219.04		75.227

				219.06		75.20908

				219.08		75.19116

				219.1		75.18519

				219.12		75.1374

				219.14		75.11947

				219.16		75.09558

				219.18		75.07168

				219.2		75.01792

				219.23		75.01195

				219.25		74.97611

				219.27		74.94624

				219.29		74.94624

				219.31		74.94026

				219.33		74.90442

				219.35		74.87455

				219.37		74.87455

				219.39		74.82079

				219.42		74.79092

				219.44		74.76105

				219.46		74.7491

				219.48		74.70729

				219.5		74.67742

				219.52		74.65352

				219.54		74.64755

				219.56		74.61171

				219.58		74.59976

				219.6		74.59379

				219.63		74.55795

				219.65		74.5221

				219.67		74.50418

				219.69		74.47431

				219.71		74.42652

				219.73		74.42055

				219.75		74.40263

				219.77		74.37276

				219.79		74.34886

				219.81		74.34886

				219.84		74.2951

				219.86		74.26523

				219.88		74.26523

				219.9		74.22939

				219.92		74.19952

				219.94		74.19355

				219.96		74.16965

				219.98		74.12186

				220		74.10394

				220.02		74.07407

				220.05		74.04421

				220.07		74.00239

				220.09		73.99044

				220.11		73.96655

				220.13		73.93668

				220.15		73.92473

				220.17		73.91876

				220.19		73.88889

				220.21		73.85902

				220.24		73.83513

				220.26		73.81123

				220.28		73.77539

				220.3		73.75747

				220.32		73.75149

				220.34		73.70968

				220.36		73.67981

				220.38		73.66189

				220.4		73.63202

				220.42		73.59618

				220.45		73.60215

				220.47		73.57228

				220.49		73.53047

				220.51		73.51254

				220.53		73.49462

				220.55		73.44683

				220.57		73.41697

				220.59		73.41099

				220.61		73.37515

				220.63		73.33931

				220.66		73.30944

				220.68		73.28554

				220.7		73.23775

				220.72		73.20789

				220.74		73.20789

				220.76		73.18399

				220.78		73.1601

				220.8		73.14815

				220.82		73.13023

				220.84		73.07049

				220.87		73.05257

				220.89		73.0227

				220.91		73.00478

				220.93		72.96296

				220.95		72.94504

				220.97		72.91517

				220.99		72.8853

				221.01		72.84349

				221.03		72.83154

				221.06		72.80765

				221.08		72.7718

				221.1		72.74791

				221.12		72.72401

				221.14		72.67622

				221.16		72.65233

				221.18		72.62843

				221.2		72.61051

				221.22		72.58065

				221.24		72.57467

				221.27		72.53883

				221.29		72.52091

				221.31		72.47909

				221.33		72.47312

				221.35		72.42533

				221.37		72.40143

				221.39		72.37754

				221.41		72.3417

				221.43		72.30585

				221.45		72.29391

				221.48		72.27599

				221.5		72.2282

				221.52		72.21625

				221.54		72.19235

				221.56		72.15054

				221.58		72.12067

				221.6		72.10872

				221.62		72.07885

				221.64		72.03106

				221.67		72.01314

				221.69		72.00119

				221.71		71.96535

				221.73		71.92354

				221.75		71.91159

				221.77		71.88769

				221.79		71.84588

				221.81		71.81601

				221.83		71.81004

				221.85		71.76822

				221.88		71.73835

				221.9		71.70251

				221.92		71.68459

				221.94		71.6368

				221.96		71.62485

				221.98		71.60096

				222		71.58303

				222.02		71.55317

				222.04		71.53524

				222.07		71.51135

				222.09		71.48148

				222.11		71.45161

				222.13		71.43369

				222.15		71.40382

				222.17		71.37395

				222.19		71.35006

				222.21		71.32616

				222.23		71.28435

				222.26		71.26045

				222.28		71.21864

				222.3		71.1828

				222.32		71.15293

				222.34		71.14098

				222.36		71.10514

				222.38		71.08124

				222.4		71.0454

				222.42		71.02748

				222.44		70.97969

				222.47		70.95579

				222.49		70.91995

				222.51		70.90203

				222.53		70.86022

				222.55		70.85424

				222.57		70.83035

				222.59		70.80645

				222.61		70.7945

				222.63		70.77061

				222.65		70.72879

				222.68		70.68698

				222.7		70.66308

				222.72		70.62127

				222.74		70.58542

				222.76		70.58542

				222.78		70.56153

				222.8		70.52569

				222.82		70.48984

				222.84		70.48387

				222.87		70.43011

				222.89		70.41219

				222.91		70.37634

				222.93		70.37037

				222.95		70.32855

				222.97		70.30466

				222.99		70.27479

				223.01		70.26284

				223.03		70.20908

				223.05		70.19116

				223.08		70.15532

				223.1		70.10753

				223.12		70.08363

				223.14		70.05974

				223.16		70.01792

				223.18		69.98208

				223.2		69.98208

				223.22		69.94026

				223.24		69.91039

				223.27		69.88053

				223.29		69.87455

				223.31		69.82676

				223.33		69.78495

				223.35		69.75508

				223.37		69.73716

				223.39		69.70131

				223.41		69.67145

				223.43		69.66547

				223.45		69.6356

				223.48		69.59976

				223.5		69.546

				223.52		69.52808

				223.54		69.50418

				223.56		69.48029

				223.58		69.45639

				223.6		69.44444

				223.62		69.40263

				223.64		69.36679

				223.67		69.32497

				223.69		69.2951

				223.71		69.26523

				223.73		69.23536

				223.75		69.19952

				223.77		69.16965

				223.79		69.15173

				223.81		69.12186

				223.83		69.07407

				223.85		69.04421

				223.88		69.03226

				223.9		68.98447

				223.92		68.96057

				223.94		68.9546

				223.96		68.91876

				223.98		68.86499

				224		68.8411

				224.02		68.79331

				224.04		68.75747

				224.07		68.73357

				224.09		68.7276

				224.11		68.68578

				224.13		68.68578

				224.15		68.64994

				224.17		68.60215

				224.19		68.56631

				224.21		68.53644

				224.23		68.49462

				224.25		68.45281

				224.28		68.44086

				224.3		68.41697

				224.32		68.3871

				224.34		68.35125

				224.36		68.33931

				224.38		68.30346

				224.4		68.26762

				224.42		68.23775

				224.44		68.22581

				224.47		68.18399

				224.49		68.15412

				224.51		68.11828

				224.53		68.08841

				224.55		68.04062

				224.57		68.01673

				224.59		67.96894

				224.61		67.95102

				224.63		67.92712

				224.65		67.9092

				224.68		67.85544

				224.7		67.83751

				224.72		67.82557

				224.74		67.7957

				224.76		67.75388

				224.78		67.74194

				224.8		67.71804

				224.82		67.66428

				224.84		67.64038

				224.87		67.62843

				224.89		67.59259

				224.91		67.56272

				224.93		67.52091

				224.95		67.49701

				224.97		67.44325

				224.99		67.41935

				225.01		67.38949

				225.03		67.35962

				225.05		67.31183

				225.08		67.28793

				225.1		67.24612

				225.12		67.21625

				225.14		67.19833

				225.16		67.18041

				225.18		67.12664

				225.2		67.08483

				225.22		67.06691

				225.24		67.02509

				225.27		66.98925

				225.29		66.95938

				225.31		66.95938

				225.33		66.89964

				225.35		66.86977

				225.37		66.84588

				225.39		66.81601

				225.41		66.76822

				225.43		66.74432

				225.46		66.72043

				225.48		66.67264

				225.5		66.66069

				225.52		66.6368

				225.54		66.58901

				225.56		66.53524

				225.58		66.51135

				225.6		66.45759

				225.62		66.41577

				225.64		66.39785

				225.67		66.37395

				225.69		66.33811

				225.71		66.31422

				225.73		66.29032

				225.75		66.24851

				225.77		66.21266

				225.79		66.1828

				225.81		66.17682

				225.83		66.13501

				225.86		66.11708

				225.88		66.09916

				225.9		66.0454

				225.92		65.99761

				225.94		65.96177

				225.96		65.9319

				225.98		65.87216

				226		65.86022

				226.02		65.81243

				226.04		65.77658

				226.07		65.74074

				226.09		65.72879

				226.11		65.681

				226.13		65.63919

				226.15		65.63321

				226.17		65.58542

				226.19		65.54958

				226.21		65.53763

				226.23		65.52569

				226.26		65.47192

				226.28		65.43011

				226.3		65.39427

				226.32		65.35245

				226.34		65.29869

				226.36		65.29271

				226.38		65.26882

				226.4		65.23297

				226.42		65.20311

				226.44		65.19116

				226.47		65.15532

				226.49		65.11947

				226.51		65.09558

				226.53		65.05974

				226.55		64.99403

				226.57		64.96416

				226.59		64.94026

				226.61		64.91039

				226.63		64.85066

				226.65		64.85663

				226.68		64.80287

				226.7		64.76703

				226.72		64.73118

				226.74		64.72521

				226.76		64.66547

				226.78		64.62963

				226.8		64.61171

				226.82		64.56989

				226.84		64.53405

				226.86		64.49821

				226.89		64.47431

				226.91		64.41458

				226.93		64.39068

				226.95		64.34886

				226.97		64.33094

				226.99		64.28913

				227.01		64.27718

				227.03		64.22939

				227.05		64.19355

				227.07		64.15173

				227.1		64.12784

				227.12		64.08602

				227.14		64.0681

				227.16		64.04421

				227.18		63.99642

				227.2		63.97252

				227.22		63.94265

				227.24		63.91876

				227.26		63.87694

				227.28		63.84707

				227.31		63.81123

				227.33		63.76344

				227.35		63.70968

				227.37		63.67981

				227.39		63.64397

				227.41		63.58423

				227.43		63.55436

				227.45		63.51852

				227.47		63.48865

				227.5		63.45878

				227.52		63.44683

				227.54		63.41697

				227.56		63.38112

				227.58		63.35723

				227.6		63.30346

				227.62		63.26165

				227.64		63.22581

				227.66		63.20789

				227.68		63.15412

				227.71		63.1362

				227.73		63.11231

				227.75		63.08841

				227.77		63.04062

				227.79		63.01673

				227.81		62.96894

				227.83		62.92712

				227.85		62.8853

				227.87		62.83751

				227.89		62.80167

				227.92		62.75986

				227.94		62.73596

				227.96		62.70609

				227.98		62.6822

				228		62.64636

				228.02		62.62246

				228.04		62.57467

				228.06		62.53286

				228.08		62.50896

				228.1		62.47909

				228.13		62.42533

				228.15		62.40143

				228.17		62.37754

				228.19		62.32378

				228.21		62.29391

				228.23		62.26404

				228.25		62.24014

				228.27		62.18638

				228.29		62.16846

				228.31		62.12067

				228.34		62.09677

				228.36		62.04898

				228.38		62.01912

				228.4		61.96535

				228.42		61.93548

				228.44		61.89964

				228.46		61.85783

				228.48		61.82796

				228.5		61.79809

				228.53		61.75627

				228.55		61.70848

				228.57		61.68459

				228.59		61.64277

				228.61		61.6129

				228.63		61.58901

				228.65		61.55317

				228.67		61.5233

				228.69		61.48148

				228.71		61.45759

				228.74		61.39785

				228.76		61.36798

				228.78		61.32019

				228.8		61.29032

				228.82		61.24253

				228.84		61.21266

				228.86		61.1828

				228.88		61.14098

				228.9		61.09916

				228.92		61.05137

				228.95		61.02151

				228.97		60.97372

				228.99		60.94385

				229.01		60.91398

				229.03		60.88411

				229.05		60.86022

				229.07		60.81243

				229.09		60.78853

				229.11		60.74074

				229.13		60.71087

				229.16		60.65711

				229.18		60.62724

				229.2		60.58542

				229.22		60.54958

				229.24		60.50777

				229.26		60.46595

				229.28		60.43608

				229.3		60.40621

				229.32		60.37037

				229.34		60.33453

				229.37		60.29869

				229.39		60.25687

				229.41		60.20908

				229.43		60.18519

				229.45		60.14934

				229.47		60.11947

				229.49		60.08363

				229.51		60.04779

				229.53		60

				229.55		59.96416

				229.58		59.92832

				229.6		59.88053

				229.62		59.84468

				229.64		59.80884

				229.66		59.773

				229.68		59.73118

				229.7		59.70729

				229.72		59.67145

				229.74		59.62366

				229.77		59.59976

				229.79		59.55795

				229.81		59.51016

				229.83		59.45042

				229.85		59.42055

				229.87		59.36679

				229.89		59.33692

				229.91		59.30108

				229.93		59.27121

				229.95		59.22939

				229.98		59.18757

				230		59.15173

				230.02		59.10394

				230.04		59.07407

				230.06		59.03226

				230.08		59.01434

				230.1		58.96057

				230.12		58.9307

				230.14		58.88889

				230.16		58.87097

				230.19		58.8172

				230.21		58.79331

				230.23		58.75747

				230.25		58.72162

				230.27		58.67384

				230.29		58.62605

				230.31		58.58423

				230.33		58.56631

				230.35		58.53047

				230.37		58.48865

				230.4		58.46476

				230.42		58.42891

				230.44		58.36918

				230.46		58.33931

				230.48		58.28554

				230.5		58.2497

				230.52		58.20789

				230.54		58.17802

				230.56		58.12425

				230.58		58.11828

				230.61		58.07646

				230.63		58.04659

				230.65		57.98686

				230.67		57.96894

				230.69		57.9092

				230.71		57.86141

				230.73		57.83751

				230.75		57.80765

				230.77		57.75388

				230.79		57.71804

				230.82		57.70012

				230.84		57.63441

				230.86		57.60454

				230.88		57.55078

				230.9		57.51493

				230.92		57.46117

				230.94		57.4313

				230.96		57.38351

				230.98		57.34767

				231		57.30585

				231.03		57.26404

				231.05		57.23417

				231.07		57.18041

				231.09		57.14456

				231.11		57.1147

				231.13		57.07885

				231.15		57.01912

				231.17		57.01314

				231.19		56.96535

				231.21		56.91159

				231.24		56.86977

				231.26		56.8399

				231.28		56.77419

				231.3		56.7503

				231.32		56.71446

				231.34		56.67861

				231.36		56.63082

				231.38		56.58901

				231.4		56.55317

				231.43		56.51732

				231.45		56.46356

				231.47		56.43369

				231.49		56.40382

				231.51		56.35603

				231.53		56.30824

				231.55		56.27838

				231.57		56.23059

				231.59		56.17085

				231.61		56.13501

				231.64		56.08722

				231.66		56.05137

				231.68		56.00956

				231.7		55.99164

				231.72		55.94982

				231.74		55.91398

				231.76		55.87216

				231.78		55.83632

				231.8		55.78256

				231.82		55.75269

				231.85		55.71685

				231.87		55.67503

				231.89		55.63919

				231.91		55.58542

				231.93		55.53763

				231.95		55.48984

				231.97		55.44803

				231.99		55.43608

				232.01		55.38829

				232.03		55.35842

				232.06		55.31661

				232.08		55.26284

				232.1		55.19713

				232.12		55.18519

				232.14		55.12545

				232.16		55.08961

				232.18		55.05974

				232.2		55.01195

				232.22		54.95818

				232.25		54.93429

				232.27		54.8865

				232.29		54.84468

				232.31		54.80287

				232.33		54.77897

				232.35		54.73118

				232.37		54.66547

				232.39		54.6356

				232.41		54.58781

				232.43		54.546

				232.46		54.47431

				232.48		54.45639

				232.5		54.4086

				232.52		54.37276

				232.54		54.33094

				232.56		54.31302

				232.58		54.24134

				232.6		54.2055

				232.62		54.17563

				232.64		54.11589

				232.67		54.06213

				232.69		54.05018

				232.71		53.99642

				232.73		53.9307

				232.75		53.90084

				232.77		53.87694

				232.79		53.83513

				232.81		53.80526

				232.83		53.78136

				232.85		53.72162

				232.88		53.67981

				232.9		53.63202

				232.92		53.5902

				232.94		53.53644

				232.96		53.51254

				232.98		53.47073

				233		53.41099

				233.02		53.37515

				233.04		53.32139

				233.06		53.2736

				233.09		53.22581

				233.11		53.18399

				233.13		53.1362

				233.15		53.09438

				233.17		53.05257

				233.19		53.03465

				233.21		52.99283

				233.23		52.94504

				233.25		52.9092

				233.27		52.86141

				233.3		52.7957

				233.32		52.75388

				233.34		52.71804

				233.36		52.67622

				233.38		52.62246

				233.4		52.58662

				233.42		52.5448

				233.44		52.49104

				233.46		52.44325

				233.48		52.41338

				233.51		52.35364

				233.53		52.30585

				233.55		52.26404

				233.57		52.23417

				233.59		52.19833

				233.61		52.16846

				233.63		52.12067

				233.65		52.07885

				233.67		52.02509

				233.69		51.98925

				233.72		51.93548

				233.74		51.90562

				233.76		51.86977

				233.78		51.82796

				233.8		51.78017

				233.82		51.74432

				233.84		51.69654

				233.86		51.66667

				233.88		51.60693

				233.9		51.55914

				233.93		51.50538

				233.95		51.45759

				233.97		51.40382

				233.99		51.37993

				234.01		51.32019

				234.03		51.29032

				234.05		51.24851

				234.07		51.19474

				234.09		51.14098

				234.11		51.09916

				234.14		51.06332

				234.16		51.00358

				234.18		50.96177

				234.2		50.9319

				234.22		50.89008

				234.24		50.83632

				234.26		50.81243

				234.28		50.76464

				234.3		50.7049

				234.32		50.66906

				234.35		50.62724

				234.37		50.5675

				234.39		50.53763

				234.41		50.50179

				234.43		50.44205

				234.45		50.39427

				234.47		50.35842

				234.49		50.31063

				234.51		50.24492

				234.53		50.21505

				234.56		50.17324

				234.58		50.12545

				234.6		50.08961

				234.62		50.05974

				234.64		50.01792

				234.66		49.97013

				234.68		49.93429

				234.7		49.87455

				234.72		49.82079

				234.74		49.76703

				234.77		49.73716

				234.79		49.70131

				234.81		49.65352

				234.83		49.62366

				234.85		49.58781

				234.87		49.51016

				234.89		49.45042

				234.91		49.41458

				234.93		49.35484

				234.95		49.2951

				234.98		49.27718

				235		49.22939

				235.02		49.17563

				235.04		49.13381

				235.06		49.09797

				235.08		49.05018

				235.1		49.00836

				235.12		48.96655

				235.14		48.91876

				235.16		48.87097

				235.19		48.8172

				235.21		48.77539

				235.23		48.70968

				235.25		48.66786

				235.27		48.62605

				235.29		48.5902

				235.31		48.53644

				235.33		48.51254

				235.35		48.46476

				235.38		48.40502

				235.4		48.3632

				235.42		48.30944

				235.44		48.26165

				235.46		48.20191

				235.48		48.17802

				235.5		48.13023

				235.52		48.08841

				235.54		48.03465

				235.56		48.01673

				235.59		47.95699

				235.61		47.90323

				235.63		47.86738

				235.65		47.82557

				235.67		47.7718

				235.69		47.71804

				235.71		47.67025

				235.73		47.61051

				235.75		47.57467

				235.77		47.52688

				235.8		47.49701

				235.82		47.44325

				235.84		47.40143

				235.86		47.32378

				235.88		47.28196

				235.9		47.21625

				235.92		47.18041

				235.94		47.12067

				235.96		47.07885

				235.98		47.03704

				236.01		46.98925

				236.03		46.94146

				236.05		46.89964

				236.07		46.8638

				236.09		46.79809

				236.11		46.7503

				236.13		46.70848

				236.15		46.67264

				236.17		46.62485

				236.19		46.57706

				236.22		46.53524

				236.24		46.47551

				236.26		46.42174

				236.28		46.36798

				236.3		46.32616

				236.32		46.2724

				236.34		46.23656

				236.36		46.17682

				236.38		46.13501

				236.4		46.08722

				236.43		46.0454

				236.45		45.97372

				236.47		45.93787

				236.49		45.88411

				236.51		45.84229

				236.53		45.7945

				236.55		45.74671

				236.57		45.7049

				236.59		45.65711

				236.61		45.59737

				236.63		45.53763

				236.66		45.50179

				236.68		45.43608

				236.7		45.40621

				236.72		45.3644

				236.74		45.3405

				236.76		45.29869

				236.78		45.24492

				236.8		45.20311

				236.82		45.14934

				236.84		45.08363

				236.87		45.01792

				236.89		44.98805

				236.91		44.91637

				236.93		44.88053

				236.95		44.83274

				236.97		44.77897

				236.99		44.73118

				237.01		44.68937

				237.03		44.61171

				237.05		44.55795

				237.08		44.5221

				237.1		44.46834

				237.12		44.4086

				237.14		44.39068

				237.16		44.34886

				237.18		44.2951

				237.2		44.24731

				237.22		44.21147

				237.24		44.15173

				237.27		44.10394

				237.29		44.05615

				237.31		44.00239

				237.33		43.96057

				237.35		43.91278

				237.37		43.85902

				237.39		43.79928

				237.41		43.74552

				237.43		43.69773

				237.45		43.64397

				237.48		43.59618

				237.5		43.55436

				237.52		43.5006

				237.54		43.44086

				237.56		43.3871

				237.58		43.37515

				237.6		43.32139

				237.62		43.26165

				237.64		43.21983

				237.66		43.17802

				237.69		43.10036

				237.71		43.04659

				237.73		43.02867

				237.75		42.97491

				237.77		42.92712

				237.79		42.87933

				237.81		42.82557

				237.83		42.7718

				237.85		42.72999

				237.87		42.68817

				237.9		42.63441

				237.92		42.59857

				237.94		42.5448

				237.96		42.48507

				237.98		42.42533

				238		42.38351

				238.02		42.32378

				238.04		42.26404

				238.06		42.22222

				238.08		42.18638

				238.11		42.13262

				238.13		42.07288

				238.15		42.03704

				238.17		41.98925

				238.19		41.91159

				238.21		41.85185

				238.23		41.81004

				238.25		41.73835

				238.27		41.68459

				238.29		41.6368

				238.32		41.58901

				238.34		41.54122

				238.36		41.49343

				238.38		41.43967

				238.4		41.3859

				238.42		41.33214

				238.44		41.29032

				238.46		41.23656

				238.48		41.16487

				238.5		41.13501

				238.53		41.08124

				238.55		41.00956

				238.57		40.97372

				238.59		40.94385

				238.61		40.87216

				238.63		40.81243

				238.65		40.77658

				238.67		40.72879

				238.69		40.67503

				238.72		40.62127

				238.74		40.5914

				238.76		40.53166

				238.78		40.46595

				238.8		40.41219

				238.82		40.37037

				238.84		40.30466

				238.86		40.26284

				238.88		40.21505

				238.9		40.15532

				238.93		40.09558

				238.95		40.04779

				238.97		39.98805

				238.99		39.91637

				239.01		39.89247

				239.03		39.83274

				239.05		39.773

				239.07		39.71924

				239.09		39.70131

				239.11		39.62963

				239.14		39.58781

				239.16		39.55197

				239.18		39.49821

				239.2		39.4325

				239.22		39.38471

				239.24		39.33692

				239.26		39.27121

				239.28		39.22939

				239.3		39.19355

				239.32		39.11589

				239.35		39.06213

				239.37		39.00836

				239.39		38.93668

				239.41		38.87097

				239.43		38.83513

				239.45		38.78734

				239.47		38.73357

				239.49		38.67384

				239.51		38.63799

				239.53		38.57826

				239.56		38.5006

				239.58		38.45878

				239.6		38.41697

				239.62		38.35125

				239.64		38.30346

				239.66		38.26762

				239.68		38.20789

				239.7		38.18996

				239.72		38.08244

				239.74		37.86738

				239.77		37.63441

				239.79		37.43728

				239.81		37.31183

				239.83		37.32975

				239.85		37.44922

				239.87		37.56272

				239.89		37.61649

				239.91		37.57467

				239.93		37.49104

				239.95		37.41935

				239.97		37.37157

				240		37.32378

				240.02		37.32378

				240.04		37.27599

				240.06		37.2282

				240.08		37.16846

				240.1		37.15054

				240.12		37.09677

				240.14		37.05496

				240.16		37.00717

				240.18		36.95938

				240.21		36.91159

				240.23		36.92951

				240.25		36.96535

				240.27		37.00119

				240.29		37.05496

				240.31		37.06691

				240.33		36.9773

				240.35		36.88769

				240.37		36.76822

				240.39		36.6129

				240.42		36.46953

				240.44		36.36798

				240.46		36.24851

				240.48		36.1589

				240.5		36.10514

				240.52		36.05137

				240.54		35.97969

				240.56		35.91995

				240.58		35.87814

				240.6		35.82437

				240.63		35.75866

				240.65		35.7049

				240.67		35.65711

				240.69		35.60335

				240.71		35.53763

				240.73		35.4779

				240.75		35.43608

				240.77		35.38232

				240.79		35.32258

				240.81		35.26284

				240.84		35.21505

				240.86		35.14934

				240.88		35.10155

				240.9		35.03584

				240.92		35

				240.94		34.95221

				240.96		34.90442

				240.98		34.83871

				241		34.77897

				241.03		34.73118

				241.05		34.65352

				241.07		34.60573

				241.09		34.546

				241.11		34.50418

				241.13		34.42652

				241.15		34.38471

				241.17		34.31302

				241.19		34.27718

				241.21		34.21744

				241.24		34.17563

				241.26		34.10992

				241.28		34.06213

				241.3		34.00836

				241.32		33.94265

				241.34		33.88889

				241.36		33.83513

				241.38		33.76941

				241.4		33.70968

				241.42		33.64397

				241.45		33.57826

				241.47		33.51852

				241.49		33.46476

				241.51		33.41099

				241.53		33.35723

				241.55		33.30346

				241.57		33.2497

				241.59		33.18996

				241.61		33.1362

				241.63		33.08244

				241.66		33.02867

				241.68		32.95699

				241.7		32.90323

				241.72		32.84946

				241.74		32.7957

				241.76		32.73596

				241.78		32.70012

				241.8		32.64038

				241.82		32.57467

				241.85		32.52688

				241.87		32.47312

				241.89		32.41338

				241.91		32.34767

				241.93		32.30585

				241.95		32.24612

				241.97		32.19235

				241.99		32.1147

				242.01		32.07288

				242.03		31.98925

				242.06		31.92354

				242.08		31.8638

				242.1		31.82198

				242.12		31.7503

				242.14		31.70251

				242.16		31.64277

				242.18		31.58901

				242.2		31.53524

				242.22		31.48746

				242.24		31.45161

				242.27		31.39188

				242.29		31.33214

				242.31		31.2724

				242.33		31.21266

				242.35		31.11708

				242.37		31.07527

				242.39		31.00358

				242.41		30.95579

				242.43		30.89606

				242.46		30.85424

				242.48		30.7945

				242.5		30.74671

				242.52		30.67503

				242.54		30.62724

				242.56		30.57348

				242.58		30.50777

				242.6		30.44803

				242.62		30.38232

				242.64		30.31661

				242.67		30.25687

				242.69		30.20311

				242.71		30.14934

				242.73		30.10753

				242.75		30.03584

				242.77		29.99403

				242.79		29.92832

				242.81		29.86858

				242.83		29.78495

				242.85		29.73716

				242.88		29.66547

				242.9		29.60573

				242.92		29.55197

				242.94		29.49821

				242.96		29.45639

				242.98		29.40263

				243		29.34289

				243.02		29.28913

				243.04		29.24731

				243.06		29.17563

				243.09		29.11589

				243.11		29.05615

				243.13		29.00239

				243.15		28.9307

				243.17		28.87097

				243.19		28.79928

				243.21		28.75747

				243.23		28.67981

				243.25		28.63202

				243.28		28.57228

				243.3		28.52449

				243.32		28.44683

				243.34		28.3871

				243.36		28.32736

				243.38		28.26165

				243.4		28.20789

				243.42		28.14815

				243.44		28.09438

				243.46		28.03465

				243.49		27.98088

				243.51		27.92115

				243.53		27.85544

				243.55		27.7957

				243.57		27.73596

				243.59		27.67025

				243.61		27.61051

				243.63		27.56272

				243.65		27.50299

				243.67		27.44325

				243.7		27.38949

				243.72		27.32975

				243.74		27.25806

				243.76		27.19235

				243.78		27.13262

				243.8		27.07288

				243.82		27.01314

				243.84		26.95341

				243.86		26.89367

				243.89		26.8399

				243.91		26.78614

				243.93		26.71446

				243.95		26.66667

				243.97		26.61888

				243.99		26.55317

				244.01		26.48746

				244.03		26.42772

				244.05		26.35603

				244.07		26.28435

				244.1		26.21864

				244.12		26.16487

				244.14		26.10514

				244.16		26.03943

				244.18		25.97372

				244.2		25.91995

				244.22		25.84827

				244.24		25.78853

				244.26		25.71087

				244.28		25.681

				244.31		25.60335

				244.33		25.56153

				244.35		25.48387

				244.37		25.454

				244.39		25.37037

				244.41		25.31661

				244.43		25.25687

				244.45		25.20311

				244.47		25.13142

				244.49		25.06571

				244.52		25.01195

				244.54		24.94026

				244.56		24.87455

				244.58		24.80884

				244.6		24.75508

				244.62		24.69534

				244.64		24.64158

				244.66		24.57587

				244.68		24.51613

				244.71		24.44444

				244.73		24.36081

				244.75		24.30108

				244.77		24.23536

				244.79		24.18757

				244.81		24.11589

				244.83		24.06213

				244.85		23.99642

				244.87		23.94265

				244.89		23.86499

				244.92		23.8172

				244.94		23.74552

				244.96		23.69176

				244.98		23.62605

				245		23.57228

				245.02		23.51254

				245.04		23.45878

				245.06		23.39307

				245.08		23.33931

				245.1		23.26762

				245.13		23.21386

				245.15		23.15412

				245.17		23.08244

				245.19		23.00478

				245.21		22.97491

				245.23		22.89725

				245.25		22.83751

				245.27		22.7718

				245.29		22.72401

				245.31		22.63441

				245.34		22.58065

				245.36		22.50299

				245.38		22.44922

				245.4		22.39546

				245.42		22.33572

				245.44		22.26404

				245.46		22.2282

				245.48		22.16249

				245.5		22.10872

				245.53		22.04301

				245.55		21.98925

				245.57		21.92951

				245.59		21.8638

				245.61		21.78614

				245.63		21.7503

				245.65		21.69654

				245.67		21.61888

				245.69		21.54719

				245.71		21.49343

				245.74		21.40382

				245.76		21.34409

				245.78		21.28435

				245.8		21.23656

				245.82		21.17085

				245.84		21.11111

				245.86		21.02748

				245.88		20.96774

				245.9		20.87814

				245.93		20.82437

				245.95		20.74671

				245.97		20.69892

				245.99		20.62724

				246.01		20.57348

				246.03		20.50179

				246.05		20.45998

				246.07		20.38829

				246.09		20.32258

				246.11		20.26284

				246.14		20.20908

				246.16		20.1374

				246.18		20.08363

				246.2		20.01195

				246.22		19.95221

				246.24		19.89247

				246.26		19.82676

				246.28		19.76105

				246.3		19.70729

				246.32		19.64755

				246.35		19.58184

				246.37		19.49821

				246.39		19.42652

				246.41		19.37276

				246.43		19.31302

				246.45		19.24134

				246.47		19.19952

				246.49		19.14576

				246.51		19.08005

				246.54		19.00239

				246.56		18.9546

				246.58		18.88292

				246.6		18.80526

				246.62		18.73357

				246.64		18.69773

				246.66		18.6141

				246.68		18.55436

				246.7		18.50657

				246.72		18.44683

				246.75		18.37515

				246.77		18.31541

				246.79		18.25568

				246.81		18.18996

				246.83		18.13023

				246.85		18.06452

				246.87		18.00478

				246.89		17.92115

				246.91		17.86141

				246.94		17.7957

				246.96		17.71804

				246.98		17.65233

				247		17.62246

				247.02		17.5448

				247.04		17.47312

				247.06		17.41935

				247.08		17.35962

				247.1		17.27001

				247.12		17.19833

				247.15		17.15651

				247.17		17.0908

				247.19		17.02509

				247.21		16.97133

				247.23		16.91159

				247.25		16.83393

				247.27		16.76225

				247.29		16.69056

				247.31		16.6129

				247.33		16.52927

				247.36		16.46953

				247.38		16.4098

				247.4		16.35603

				247.42		16.30227

				247.44		16.26045

				247.46		16.18877

				247.48		16.12306

				247.5		16.06332

				247.52		15.98566

				247.55		15.91398

				247.57		15.85424

				247.59		15.7945

				247.61		15.71685

				247.63		15.65711

				247.65		15.58542

				247.67		15.51971

				247.69		15.454

				247.71		15.38232

				247.73		15.32258

				247.76		15.26284

				247.78		15.20311

				247.8		15.1374

				247.82		15.07168

				247.84		15.01195

				247.86		14.95221

				247.88		14.8865

				247.9		14.81481

				247.92		14.76105

				247.95		14.68339

				247.97		14.60573

				247.99		14.54002

				248.01		14.48626

				248.03		14.41458

				248.05		14.34886

				248.07		14.2951

				248.09		14.23536

				248.11		14.16368

				248.13		14.10992

				248.16		14.03226

				248.18		13.96057

				248.2		13.88292

				248.22		13.82915

				248.24		13.74552

				248.26		13.7037

				248.28		13.64994

				248.3		13.57826

				248.32		13.51254

				248.35		13.47073

				248.37		13.39307

				248.39		13.32736

				248.41		13.26165

				248.43		13.20191

				248.45		13.11828

				248.47		13.05257

				248.49		12.98686

				248.51		12.91517

				248.53		12.84349

				248.56		12.78375

				248.58		12.72999

				248.6		12.6583

				248.62		12.59857

				248.64		12.53286

				248.66		12.46714

				248.68		12.37754

				248.7		12.3178

				248.72		12.26404

				248.75		12.17443

				248.77		12.13262

				248.79		12.07288

				248.81		11.99522

				248.83		11.92354

				248.85		11.87575

				248.87		11.77419

				248.89		11.70848

				248.91		11.64277

				248.94		11.59498

				248.96		11.53524

				248.98		11.46953

				249		11.4098

				249.02		11.35603

				249.04		11.2724

				249.06		11.18877

				249.08		11.12903

				249.1		11.05137

				249.12		10.98566

				249.15		10.91995

				249.17		10.87216

				249.19		10.80645

				249.21		10.74074

				249.23		10.66906

				249.25		10.60335

				249.27		10.53166

				249.29		10.454

				249.31		10.39427

				249.34		10.31661

				249.36		10.26284

				249.38		10.20311

				249.4		10.1374

				249.42		10.07168

				249.44		10.01195

				249.46		9.922342

				249.48		9.856631

				249.5		9.796894

				249.52		9.737157

				249.55		9.671446

				249.57		9.617682

				249.59		9.545998

				249.61		9.504182

				249.63		9.426523

				249.65		9.354839

				249.67		9.283154

				249.69		9.217443

				249.71		9.139785

				249.74		9.080048

				249.76		9.008363

				249.78		8.966547

				249.8		8.90681

				249.82		8.841099

				249.84		8.769415

				249.86		8.727599

				249.88		8.64994

				249.9		8.572282

				249.92		8.506571

				249.95		8.458781

				249.97		8.387097

				249.99		8.321386

				250.01		8.273596

				250.03		8.207885

				250.05		8.11828

				250.07		8.064516

				250.09		7.992832

				250.11		7.927121

				250.13		7.897252

				250.16		7.915173

				250.18		7.801673

				250.2		7.759857

				250.22		7.670251

				250.24		7.562724

				250.26		7.407407

				250.28		7.383513

				250.3		7.287933

				250.32		7.23417

				250.35		7.174432

				250.37		7.120669

				250.39		7.054958

				250.41		7.001195

				250.43		6.935484

				250.45		6.875747

				250.47		6.810036

				250.49		6.76822

				250.51		6.684588

				250.53		6.666667

				250.56		6.589008

				250.58		6.55914

				250.6		6.439665

				250.62		6.391876

				250.64		6.290323

				250.66		6.218638

				250.68		6.123059

				250.7		6.105137

				250.72		6.027479

				250.74		5.949821

				250.77		5.878136

				250.79		5.758662

				250.81		5.716846

				250.83		5.770609

				250.85		5.57945

				250.87		5.561529

				250.89		5.561529

				250.91		5.495818

				250.93		5.316607

				250.96		5.388292

				250.98		5.304659

				251		5.238949

				251.02		5.137395

				251.04		5.095579

				251.06		5.041816

				251.08		4.982079

				251.1		4.922342

				251.12		4.856631

				251.14		4.778973

				251.17		4.731183

				251.19		4.647551

				251.21		4.58184

				251.23		4.522103

				251.25		4.480287

				251.27		4.384707

				251.29		4.330944

				251.31		4.265233

				251.33		4.205496

				251.35		4.11589

				251.38		4.062127

				251.4		4.014337

				251.42		3.948626

				251.44		3.888889

				251.46		3.847073

				251.48		3.799283

				251.5		3.721625

				251.52		3.661888

				251.54		3.590203

				251.57		3.530466

				251.59		3.464755

				251.61		3.410992

				251.63		3.363202

				251.65		3.291517

				251.67		3.261649

				251.69		3.201912

				251.71		3.130227

				251.73		3.07049

				251.75		3.034648

				251.78		2.945042

				251.8		2.891278

				251.82		2.837515

				251.84		2.783751

				251.86		2.718041

				251.88		2.688172

				251.9		2.622461

				251.92		2.580645

				251.94		2.520908

				251.96		2.479092

				251.99		2.413381

				252.01		2.365591

				252.03		2.311828

				252.05		2.275986

				252.07		2.210275

				252.09		2.162485

				252.11		2.132616

				252.13		2.078853

				252.15		2.037037

				252.17		2.013142

				252.2		1.9773

				252.22		1.92951

				252.24		1.899642

				252.26		1.869773

				252.28		1.821983

				252.3		1.792115

				252.32		1.780167

				252.34		1.762246

				252.36		1.732378

				252.38		1.72043

				252.41		1.72043

				252.43		1.708483

				252.45		1.696535

				252.47		1.678614

				252.49		1.642772

				252.51		1.60693

				252.53		1.55914

				252.55		1.529271

				252.57		1.493429

				252.6		1.517324

				252.62		1.505376

				252.64		1.499403

				252.66		1.481481

				252.68		1.505376

				252.7		1.469534

				252.72		1.451613

				252.74		1.439665

				252.76		1.445639

				252.78		1.421744

				252.81		1.421744

				252.83		1.403823

				252.85		1.415771

				252.87		1.385902

				252.89		1.379928

				252.91		1.362007

				252.93		1.356033

				252.95		1.362007

				252.97		1.344086

				252.99		1.35006

				253.02		1.356033

				253.04		1.356033

				253.06		1.326165

				253.08		1.290323

				253.1		1.338112

				253.12		1.290323

				253.14		1.320191

				253.16		1.320191

				253.18		1.314217

				253.2		1.30227

				253.22		1.30227

				253.25		1.308244

				253.27		1.308244

				253.29		1.332139

				253.31		1.332139

				253.33		1.308244

				253.35		1.332139

				253.37		1.320191

				253.39		1.30227

				253.41		1.30227

				253.43		1.296296

				253.46		1.296296

				253.48		1.296296

				253.5		1.290323

				253.52		1.284349

				253.54		1.284349

				253.56		1.284349

				253.58		1.290323

				253.6		1.266428

				253.62		1.212664

				253.64		1.194743

				253.67		1.194743

				253.69		1.194743

				253.71		1.194743

				253.73		1.200717

				253.75		1.200717

				253.77		1.200717

				253.79		1.206691

				253.81		1.212664

				253.83		1.212664

				253.85		1.212664

				253.87		1.206691

				253.9		1.206691

				253.92		1.206691

				253.94		1.206691

				253.96		1.212664

				253.98		1.230585

				254		1.242533

				254.02		1.25448

				254.04		1.248507

				254.06		1.248507

				254.08		1.248507

				254.1		1.242533

				254.12		1.242533

				254.15		1.242533

				254.17		1.242533

				254.19		1.248507

				254.21		1.25448

				254.23		1.25448

				254.25		1.248507

				254.27		1.248507

				254.29		1.248507

				254.31		1.248507

				254.33		1.242533

				254.35		1.242533

				254.38		1.242533

				254.4		1.242533

				254.42		1.242533

				254.44		1.236559

				254.46		1.248507

				254.48		1.278375

				254.5		1.290323

				254.52		1.284349

				254.54		1.284349

				254.56		1.278375

				254.58		1.278375

				254.61		1.278375

				254.63		1.272401

				254.65		1.272401

				254.67		1.266428

				254.69		1.266428

				254.71		1.266428

				254.73		1.272401

				254.75		1.272401

				254.77		1.272401

				254.79		1.272401

				254.81		1.272401

				254.84		1.266428

				254.86		1.266428

				254.88		1.266428

				254.9		1.266428

				254.92		1.260454

				254.94		1.260454

				254.96		1.260454

				254.98		1.260454

				255		1.25448

				255.02		1.260454

				255.05		1.260454

				255.07		1.260454

				255.09		1.260454

				255.11		1.260454

				255.13		1.248507

				255.15		1.230585

				255.17		1.218638

				255.19		1.206691

				255.21		1.200717

				255.23		1.200717

				255.26		1.200717

				255.28		1.200717

				255.3		1.200717

				255.32		1.200717

				255.34		1.194743

				255.36		1.200717

				255.38		1.194743

				255.4		1.194743

				255.42		1.194743

				255.44		1.194743

				255.46		1.200717

				255.49		1.194743

				255.51		1.194743

				255.53		1.194743

				255.55		1.188769

				255.57		1.188769

				255.59		1.188769

				255.61		1.188769

				255.63		1.188769

				255.65		1.188769

				255.67		1.188769

				255.7		1.188769

				255.72		1.188769

				255.74		1.182796

				255.76		1.188769

				255.78		1.182796

				255.8		1.188769

				255.82		1.188769

				255.84		1.188769

				255.86		1.182796

				255.88		1.182796

				255.9		1.182796

				255.93		1.182796

				255.95		1.182796

				255.97		1.176822

				255.99		1.176822

				256.01		1.176822

				256.03		1.176822

				256.05		1.176822

				256.07		1.176822

				256.09		1.176822

				256.11		1.176822

				256.13		1.176822

				256.16		1.176822

				256.18		1.170848

				256.2		1.176822

				256.22		1.176822

				256.24		1.176822

				256.26		1.170848

				256.28		1.170848

				256.3		1.170848

				256.32		1.176822

				256.34		1.170848

				256.36		1.176822

				256.39		1.170848

				256.41		1.164875

				256.43		1.164875

				256.45		1.164875

				256.47		1.164875

				256.49		1.164875

				256.51		1.164875

				256.53		1.164875

				256.55		1.164875

				256.57		1.164875

				256.59		1.164875

				256.62		1.164875

				256.64		1.164875

				256.66		1.164875

				256.68		1.164875

				256.7		1.164875

				256.72		1.164875

				256.74		1.164875

				256.76		1.158901

				256.78		1.158901

				256.8		1.158901

				256.82		1.158901

				256.85		1.158901

				256.87		1.158901

				256.89		1.158901

				256.91		1.158901

				256.93		1.158901

				256.95		1.158901

				256.97		1.158901

				256.99		1.158901

				257.01		1.158901

				257.03		1.158901

				257.05		1.158901

				257.08		1.158901

				257.1		1.158901

				257.12		1.158901

				257.14		1.158901

				257.16		1.164875

				257.18		1.164875

				257.2		1.158901

				257.22		1.158901

				257.24		1.164875

				257.26		1.164875

				257.28		1.164875

				257.31		1.164875

				257.33		1.158901

				257.35		1.158901

				257.37		1.158901

				257.39		1.158901

				257.41		1.158901

				257.43		1.158901

				257.45		1.158901

				257.47		1.158901

				257.49		1.158901

				257.51		1.158901

				257.54		1.158901

				257.56		1.158901

				257.58		1.158901

				257.6		1.158901

				257.62		1.158901

				257.64		1.158901

				257.66		1.158901

				257.68		1.158901

				257.7		1.158901

				257.72		1.158901

				257.74		1.158901

				257.77		1.158901

				257.79		1.158901

				257.81		1.158901

				257.83		1.158901

				257.85		1.158901

				257.87		1.158901

				257.89		1.158901

				257.91		1.158901

				257.93		1.158901

				257.95		1.158901

				257.97		1.158901

				258		1.158901

				258.02		1.158901

				258.04		1.158901

				258.06		1.158901

				258.08		1.158901

				258.1		1.158901

				258.12		1.158901

				258.14		1.158901

				258.16		1.158901

				258.18		1.158901

				258.2		1.158901

				258.22		1.158901

				258.25		1.158901

				258.27		1.152927

				258.29		1.152927

				258.31		1.152927

				258.33		1.152927

				258.35		1.152927

				258.37		1.152927

				258.39		1.152927

				258.41		1.152927

				258.43		1.152927

				258.45		1.152927

				258.48		1.158901

				258.5		1.158901

				258.52		1.158901

				258.54		1.158901

				258.56		1.158901

				258.58		1.158901

				258.6		1.158901

				258.62		1.158901

				258.64		1.152927

				258.66		1.152927

				258.68		1.152927

				258.7		1.152927

				258.73		1.152927

				258.75		1.152927

				258.77		1.152927

				258.79		1.152927

				258.81		1.152927

				258.83		1.152927

				258.85		1.152927

				258.87		1.152927

				258.89		1.152927

				258.91		1.152927

				258.93		1.152927

				258.96		1.152927

				258.98		1.152927

				259		1.152927

				259.02		1.152927

				259.04		1.146953

				259.06		1.152927

				259.08		1.146953

				259.1		1.146953

				259.12		1.146953

				259.14		1.146953

				259.16		1.146953

				259.18		1.146953

				259.21		1.146953

				259.23		1.14098

				259.25		1.14098

				259.27		1.14098

				259.29		1.14098

				259.31		1.14098

				259.33		1.14098

				259.35		1.14098

				259.37		1.14098

				259.39		1.14098

				259.41		1.14098

				259.44		1.14098

				259.46		1.14098

				259.48		1.135006

				259.5		1.135006

				259.52		1.135006

				259.54		1.135006

				259.56		1.135006

				259.58		1.135006

				259.6		1.135006

				259.62		1.135006

				259.64		1.135006

				259.66		1.135006

				259.69		1.135006

				259.71		1.135006

				259.73		1.135006

				259.75		1.135006

				259.77		1.135006

				259.79		1.135006

				259.81		1.135006

				259.83		1.135006

				259.85		1.135006

				259.87		1.135006

				259.89		1.135006

				259.92		1.135006

				259.94		1.135006

				259.96		1.135006

				259.98		1.135006

				260		1.135006

				260.02		1.135006

				260.04		1.135006

				260.06		1.135006

				260.08		1.135006

				260.1		1.135006

				260.12		1.135006

				260.15		1.135006

				260.17		1.135006

				260.19		1.135006

				260.21		1.129032

				260.23		1.129032

				260.25		1.129032

				260.27		1.129032

				260.29		1.129032

				260.31		1.129032

				260.33		1.129032

				260.35		1.129032

				260.38		1.129032

				260.4		1.129032

				260.42		1.129032

				260.44		1.129032

				260.46		1.129032

				260.48		1.129032

				260.5		1.129032

				260.52		1.129032

				260.54		1.129032

				260.56		1.129032

				260.58		1.129032

				260.6		1.129032

				260.63		1.129032

				260.65		1.129032

				260.67		1.129032

				260.69		1.129032

				260.71		1.129032

				260.73		1.129032

				260.75		1.129032

				260.77		1.129032

				260.79		1.129032

				260.81		1.129032

				260.83		1.129032

				260.86		1.129032

				260.88		1.129032

				260.9		1.129032

				260.92		1.123059

				260.94		1.123059

				260.96		1.123059

				260.98		1.123059

				261		1.123059

				261.02		1.123059

				261.04		1.123059

				261.06		1.123059

				261.09		1.123059

				261.11		1.123059

				261.13		1.123059

				261.15		1.123059

				261.17		1.123059

				261.19		1.123059

				261.21		1.123059

				261.23		1.129032

				261.25		1.123059

				261.27		1.123059

				261.29		1.123059

				261.31		1.129032

				261.34		1.123059

				261.36		1.129032

				261.38		1.123059

				261.4		1.129032

				261.42		1.129032

				261.44		1.129032

				261.46		1.129032

				261.48		1.129032

				261.5		1.129032

				261.52		1.129032

				261.54		1.129032

				261.57		1.129032

				261.59		1.129032

				261.61		1.129032

				261.63		1.129032

				261.65		1.129032

				261.67		1.129032

				261.69		1.129032

				261.71		1.123059

				261.73		1.123059

				261.75		1.123059

				261.77		1.123059

				261.79		1.123059

				261.82		1.123059

				261.84		1.123059

				261.86		1.123059

				261.88		1.123059

				261.9		1.123059

				261.92		1.123059

				261.94		1.123059

				261.96		1.123059

				261.98		1.123059

				262		1.123059

				262.02		1.123059

				262.05		1.123059

				262.07		1.123059

				262.09		1.123059

				262.11		1.123059

				262.13		1.123059

				262.15		1.123059

				262.17		1.123059

				262.19		1.123059

				262.21		1.123059

				262.23		1.123059

				262.25		1.123059

				262.27		1.123059

				262.3		1.123059

				262.32		1.123059

				262.34		1.123059

				262.36		1.123059

				262.38		1.123059

				262.4		1.123059

				262.42		1.123059

				262.44		1.123059

				262.46		1.123059

				262.48		1.123059

				262.5		1.123059

				262.53		1.123059

				262.55		1.123059

				262.57		1.123059

				262.59		1.123059

				262.61		1.123059

				262.63		1.123059

				262.65		1.123059

				262.67		1.123059

				262.69		1.123059

				262.71		1.123059

				262.73		1.123059

				262.75		1.123059

				262.78		1.123059

				262.8		1.123059

				262.82		1.123059

				262.84		1.117085

				262.86		1.123059

				262.88		1.123059

				262.9		1.123059

				262.92		1.123059

				262.94		1.123059

				262.96		1.123059

				262.98		1.123059

				263.01		1.123059

				263.03		1.123059

				263.05		1.123059

				263.07		1.123059

				263.09		1.123059

				263.11		1.123059

				263.13		1.123059

				263.15		1.123059

				263.17		1.123059

				263.19		1.123059

				263.21		1.123059

				263.24		1.123059

				263.26		1.123059

				263.28		1.123059

				263.3		1.123059

				263.32		1.123059

				263.34		1.123059

				263.36		1.123059

				263.38		1.123059

				263.4		1.123059

				263.42		1.123059

				263.44		1.123059

				263.47		1.123059

				263.49		1.117085

				263.51		1.123059

				263.53		1.117085

				263.55		1.117085

				263.57		1.123059

				263.59		1.123059

				263.61		1.123059

				263.63		1.123059

				263.65		1.123059

				263.67		1.123059

				263.7		1.123059

				263.72		1.123059

				263.74		1.123059

				263.76		1.123059

				263.78		1.123059

				263.8		1.123059

				263.82		1.123059

				263.84		1.123059

				263.86		1.123059

				263.88		1.117085

				263.9		1.117085

				263.93		1.117085

				263.95		1.123059

				263.97		1.117085

				263.99		1.123059

				264.01		1.123059

				264.03		1.117085

				264.05		1.117085

				264.07		1.117085

				264.09		1.123059

				264.11		1.117085

				264.13		1.117085

				264.16		1.117085

				264.18		1.117085

				264.2		1.117085

				264.22		1.117085

				264.24		1.117085

				264.26		1.117085

				264.28		1.117085

				264.3		1.117085

				264.32		1.117085

				264.34		1.117085

				264.36		1.117085

				264.39		1.111111

				264.41		1.111111

				264.43		1.111111

				264.45		1.111111

				264.47		1.111111

				264.49		1.111111

				264.51		1.111111

				264.53		1.111111

				264.55		1.111111

				264.57		1.111111

				264.59		1.111111

				264.62		1.111111

				264.64		1.111111

				264.66		1.111111

				264.68		1.111111

				264.7		1.105137

				264.72		1.111111

				264.74		1.105137

				264.76		1.105137

				264.78		1.105137

				264.8		1.105137

				264.82		1.105137

				264.84		1.105137

				264.87		1.105137

				264.89		1.105137

				264.91		1.105137

				264.93		1.105137

				264.95		1.105137

				264.97		1.105137

				264.99		1.105137

				265.01		1.105137

				265.03		1.105137

				265.05		1.099164

				265.07		1.105137

				265.1		1.105137

				265.12		1.099164

				265.14		1.099164

				265.16		1.099164

				265.18		1.099164

				265.2		1.099164

				265.22		1.099164

				265.24		1.099164

				265.26		1.099164

				265.28		1.099164

				265.3		1.099164

				265.33		1.099164

				265.35		1.099164

				265.37		1.099164

				265.39		1.099164

				265.41		1.09319

				265.43		1.09319

				265.45		1.09319

				265.47		1.09319

				265.49		1.09319

				265.51		1.09319

				265.53		1.09319

				265.56		1.09319

				265.58		1.09319

				265.6		1.09319

				265.62		1.09319

				265.64		1.087216

				265.66		1.09319

				265.68		1.087216

				265.7		1.087216

				265.72		1.087216

				265.74		1.087216

				265.76		1.087216

				265.79		1.087216

				265.81		1.087216

				265.83		1.087216

				265.85		1.087216

				265.87		1.087216

				265.89		1.087216

				265.91		1.087216

				265.93		1.087216

				265.95		1.087216

				265.97		1.087216

				265.99		1.087216

				266.01		1.087216

				266.04		1.087216

				266.06		1.087216

				266.08		1.087216

				266.1		1.087216

				266.12		1.087216

				266.14		1.081243

				266.16		1.081243

				266.18		1.081243

				266.2		1.081243

				266.22		1.081243

				266.24		1.081243

				266.27		1.081243

				266.29		1.081243

				266.31		1.081243

				266.33		1.081243

				266.35		1.081243

				266.37		1.081243

				266.39		1.081243

				266.41		1.081243

				266.43		1.081243

				266.45		1.081243

				266.47		1.081243

				266.49		1.081243

				266.52		1.081243

				266.54		1.081243

				266.56		1.081243

				266.58		1.081243

				266.6		1.081243

				266.62		1.081243

				266.64		1.081243

				266.66		1.081243

				266.68		1.081243

				266.7		1.081243

				266.72		1.081243

				266.74		1.081243

				266.77		1.081243

				266.79		1.081243

				266.81		1.081243

				266.83		1.081243

				266.85		1.081243

				266.87		1.081243

				266.89		1.081243

				266.91		1.081243

				266.93		1.081243

				266.95		1.081243

				266.97		1.081243

				267		1.081243

				267.02		1.081243

				267.04		1.081243

				267.06		1.081243

				267.08		1.081243

				267.1		1.081243

				267.12		1.081243

				267.14		1.081243

				267.16		1.081243

				267.18		1.075269

				267.2		1.075269

				267.22		1.075269

				267.25		1.075269

				267.27		1.075269

				267.29		1.075269

				267.31		1.075269

				267.33		1.075269

				267.35		1.075269

				267.37		1.075269

				267.39		1.075269

				267.41		1.075269

				267.43		1.075269

				267.45		1.075269

				267.48		1.075269

				267.5		1.075269

				267.52		1.075269

				267.54		1.075269

				267.56		1.081243

				267.58		1.075269

				267.6		1.075269

				267.62		1.075269

				267.64		1.075269

				267.66		1.075269

				267.68		1.075269

				267.71		1.075269

				267.73		1.075269

				267.75		1.075269

				267.77		1.075269

				267.79		1.075269

				267.81		1.075269

				267.83		1.075269

				267.85		1.075269

				267.87		1.075269

				267.89		1.075269

				267.91		1.069295

				267.94		1.069295

				267.96		1.069295

				267.98		1.069295

				268		1.069295

				268.02		1.069295

				268.04		1.069295

				268.06		1.069295

				268.08		1.069295

				268.1		1.069295

				268.12		1.069295

				268.14		1.069295

				268.17		1.069295

				268.19		1.069295

				268.21		1.069295

				268.23		1.069295

				268.25		1.069295

				268.27		1.069295

				268.29		1.069295

				268.31		1.069295

				268.33		1.069295

				268.35		1.069295

				268.37		1.069295

				268.4		1.069295

				268.42		1.069295

				268.44		1.069295

				268.46		1.069295

				268.48		1.069295

				268.5		1.069295

				268.52		1.069295

				268.54		1.069295

				268.56		1.069295

				268.58		1.069295

				268.6		1.069295

				268.63		1.069295

				268.65		1.069295

				268.67		1.069295

				268.69		1.069295

				268.71		1.069295

				268.73		1.069295

				268.75		1.069295

				268.77		1.075269

				268.79		1.075269

				268.81		1.075269

				268.83		1.075269

				268.86		1.075269

				268.88		1.075269

				268.9		1.075269

				268.92		1.069295

				268.94		1.075269

				268.96		1.075269

				268.98		1.075269

				269		1.069295

				269.02		1.069295

				269.04		1.069295

				269.06		1.069295

				269.09		1.069295

				269.11		1.069295

				269.13		1.069295

				269.15		1.069295

				269.17		1.069295

				269.19		1.069295

				269.21		1.069295

				269.23		1.069295

				269.25		1.069295

				269.27		1.069295

				269.29		1.069295

				269.31		1.069295

				269.34		1.069295

				269.36		1.069295

				269.38		1.069295

				269.4		1.069295

				269.42		1.069295

				269.44		1.069295

				269.46		1.069295

				269.48		1.069295

				269.5		1.069295

				269.52		1.069295

				269.54		1.069295

				269.57		1.069295

				269.59		1.069295

				269.61		1.069295

				269.63		1.069295

				269.65		1.069295

				269.67		1.069295

				269.69		1.069295

				269.71		1.069295

				269.73		1.069295

				269.75		1.069295

				269.77		1.069295

				269.8		1.063321

				269.82		1.069295

				269.84		1.063321

				269.86		1.069295

				269.88		1.063321

				269.9		1.063321

				269.92		1.063321

				269.94		1.063321

				269.96		1.069295

				269.98		1.069295

				270		1.069295

				270.03		1.069295

				270.05		1.069295

				270.07		1.069295

				270.09		1.069295

				270.11		1.069295

				270.13		1.069295

				270.15		1.069295

				270.17		1.069295

				270.19		1.069295

				270.21		1.069295

				270.24		1.069295

				270.26		1.069295

				270.28		1.069295

				270.3		1.063321

				270.32		1.069295

				270.34		1.063321

				270.36		1.063321

				270.38		1.063321

				270.4		1.069295

				270.42		1.063321

				270.44		1.063321

				270.47		1.063321

				270.49		1.063321

				270.51		1.063321

				270.53		1.063321

				270.55		1.063321

				270.57		1.063321

				270.59		1.057348

				270.61		1.057348

				270.63		1.057348

				270.65		1.057348

				270.67		1.057348

				270.7		1.051374

				270.72		1.051374

				270.74		1.051374

				270.76		1.051374

				270.78		1.051374

				270.8		1.051374

				270.82		1.051374

				270.84		1.051374

				270.86		1.051374

				270.88		1.051374

				270.9		1.051374

				270.93		1.051374

				270.95		1.051374

				270.97		1.0454

				270.99		1.0454

				271.01		1.0454

				271.03		1.0454

				271.05		1.0454

				271.07		1.0454

				271.09		1.0454

				271.11		1.0454

				271.14		1.0454

				271.16		1.0454

				271.18		1.0454

				271.2		1.0454

				271.22		1.0454

				271.24		1.0454

				271.26		1.0454

				271.28		1.0454

				271.3		1.0454

				271.32		1.0454

				271.34		1.0454

				271.37		1.0454

				271.39		1.0454

				271.41		1.0454

				271.43		1.0454

				271.45		1.0454

				271.47		1.0454

				271.49		1.0454

				271.51		1.0454

				271.53		1.0454

				271.55		1.0454

				271.57		1.0454

				271.6		1.0454

				271.62		1.0454

				271.64		1.0454

				271.66		1.0454

				271.68		1.039427

				271.7		1.039427

				271.72		1.039427

				271.74		1.039427

				271.76		1.039427

				271.78		1.039427

				271.81		1.039427

				271.83		1.039427

				271.85		1.039427

				271.87		1.039427

				271.89		1.039427

				271.91		1.039427

				271.93		1.039427

				271.95		1.039427

				271.97		1.039427

				271.99		1.039427

				272.01		1.039427

				272.04		1.039427

				272.06		1.039427

				272.08		1.039427

				272.1		1.039427

				272.12		1.039427

				272.14		1.039427

				272.16		1.039427

				272.18		1.039427

				272.2		1.039427

				272.22		1.039427

				272.25		1.039427

				272.27		1.039427

				272.29		1.039427

				272.31		1.039427

				272.33		1.039427

				272.35		1.039427

				272.37		1.039427

				272.39		1.039427

				272.41		1.039427

				272.43		1.039427

				272.45		1.039427

				272.48		1.039427

				272.5		1.039427

				272.52		1.039427

				272.54		1.039427

				272.56		1.039427

				272.58		1.039427

				272.6		1.039427

				272.62		1.039427

				272.64		1.039427

				272.66		1.039427

				272.68		1.039427

				272.71		1.039427

				272.73		1.039427

				272.75		1.039427

				272.77		1.039427

				272.79		1.039427

				272.81		1.039427

				272.83		1.039427

				272.85		1.0454

				272.87		1.039427

				272.89		1.039427

				272.92		1.0454

				272.94		1.0454

				272.96		1.0454

				272.98		1.0454

				273		1.039427

				273.02		1.039427

				273.04		1.039427

				273.06		1.039427

				273.08		1.039427

				273.1		1.0454

				273.12		1.039427

				273.15		1.039427

				273.17		1.0454

				273.19		1.039427

				273.21		1.039427

				273.23		1.039427

				273.25		1.039427

				273.27		1.0454

				273.29		1.039427

				273.31		1.0454

				273.33		1.039427

				273.35		1.0454

				273.38		1.039427

				273.4		1.039427

				273.42		1.0454

				273.44		1.0454

				273.46		1.0454

				273.48		1.0454

				273.5		1.0454

				273.52		1.0454

				273.54		1.0454

				273.56		1.0454

				273.59		1.0454

				273.61		1.0454

				273.63		1.0454

				273.65		1.039427

				273.67		1.039427

				273.69		1.039427

				273.71		1.039427

				273.73		1.039427

				273.75		1.039427

				273.77		1.039427

				273.79		1.039427

				273.82		1.039427

				273.84		1.039427

				273.86		1.039427

				273.88		1.039427

				273.9		1.039427

				273.92		1.039427

				273.94		1.039427

				273.96		1.039427

				273.98		1.039427

				274		1.039427

				274.03		1.039427

				274.05		1.039427

				274.07		1.039427

				274.09		1.039427

				274.11		1.039427

				274.13		1.039427

				274.15		1.039427

				274.17		1.039427

				274.19		1.039427

				274.21		1.039427

				274.23		1.039427

				274.26		1.039427

				274.28		1.039427

				274.3		1.039427

				274.32		1.039427

				274.34		1.039427

				274.36		1.039427

				274.38		1.039427

				274.4		1.039427

				274.42		1.039427

				274.44		1.039427

				274.47		1.039427

				274.49		1.039427

				274.51		1.039427

				274.53		1.039427

				274.55		1.039427

				274.57		1.039427

				274.59		1.039427

				274.61		1.039427

				274.63		1.039427

				274.65		1.039427

				274.67		1.039427

				274.7		1.039427

				274.72		1.039427

				274.74		1.039427

				274.76		1.039427

				274.78		1.039427

				274.8		1.039427

				274.82		1.039427

				274.84		1.039427

				274.86		1.039427

				274.88		1.039427

				274.91		1.039427

				274.93		1.039427

				274.95		1.033453

				274.97		1.033453

				274.99		1.033453

				275.01		1.033453

				275.03		1.033453

				275.05		1.033453

				275.07		1.033453

				275.09		1.033453

				275.12		1.033453

				275.14		1.033453

				275.16		1.033453

				275.18		1.033453

				275.2		1.033453

				275.22		1.033453

				275.24		1.033453

				275.26		1.033453

				275.28		1.033453

				275.3		1.033453

				275.32		1.033453

				275.35		1.033453

				275.37		1.033453

				275.39		1.033453

				275.41		1.033453

				275.43		1.033453

				275.45		1.033453

				275.47		1.033453

				275.49		1.033453

				275.51		1.033453

				275.53		1.027479

				275.56		1.027479

				275.58		1.027479

				275.6		1.027479

				275.62		1.027479

				275.64		1.027479

				275.66		1.027479

				275.68		1.027479

				275.7		1.027479

				275.72		1.027479

				275.74		1.027479

				275.77		1.027479

				275.79		1.027479

				275.81		1.027479

				275.83		1.027479

				275.85		1.027479

				275.87		1.027479

				275.89		1.027479

				275.91		1.027479

				275.93		1.027479

				275.95		1.027479

				275.97		1.027479

				276		1.027479

				276.02		1.027479

				276.04		1.027479

				276.06		1.027479

				276.08		1.027479

				276.1		1.027479

				276.12		1.027479

				276.14		1.027479

				276.16		1.027479

				276.18		1.027479

				276.2		1.027479

				276.23		1.027479

				276.25		1.027479

				276.27		1.027479

				276.29		1.027479

				276.31		1.027479

				276.33		1.027479

				276.35		1.027479

				276.37		1.027479

				276.39		1.027479

				276.41		1.027479

				276.44		1.021505

				276.46		1.027479

				276.48		1.021505

				276.5		1.021505

				276.52		1.021505

				276.54		1.021505

				276.56		1.021505

				276.58		1.021505

				276.6		1.021505

				276.62		1.021505

				276.64		1.021505

				276.67		1.021505

				276.69		1.021505

				276.71		1.021505

				276.73		1.021505

				276.75		1.021505

				276.77		1.021505

				276.79		1.021505

				276.81		1.021505

				276.83		1.021505

				276.85		1.021505

				276.88		1.015532

				276.9		1.015532

				276.92		1.015532

				276.94		1.015532

				276.96		1.015532

				276.98		1.015532

				277		1.021505

				277.02		1.015532

				277.04		1.015532

				277.06		1.015532

				277.08		1.015532

				277.11		1.015532

				277.13		1.015532

				277.15		1.015532

				277.17		1.015532

				277.19		1.015532

				277.21		1.015532

				277.23		1.015532

				277.25		1.015532

				277.27		1.015532

				277.29		1.015532

				277.31		1.015532

				277.34		1.015532

				277.36		1.015532

				277.38		1.015532

				277.4		1.015532

				277.42		1.015532

				277.44		1.009558

				277.46		1.009558

				277.48		1.009558

				277.5		1.009558

				277.52		1.009558

				277.55		1.009558

				277.57		1.009558

				277.59		1.009558

				277.61		1.009558

				277.63		1.009558

				277.65		1.009558

				277.67		1.009558

				277.69		1.009558

				277.71		1.009558

				277.73		1.009558

				277.76		1.003584

				277.78		1.009558

				277.8		1.003584

				277.82		1.003584

				277.84		1.009558

				277.86		1.003584

				277.88		1.003584

				277.9		1.003584

				277.92		1.003584

				277.94		1.003584

				277.96		1.003584

				277.99		1.003584

				278.01		1.003584

				278.03		1.003584

				278.05		1.003584

				278.07		1.003584

				278.09		1.003584

				278.11		1.003584

				278.13		1.003584

				278.15		1.003584

				278.17		1.003584

				278.2		1.003584

				278.22		1.003584

				278.24		1.003584

				278.26		1.003584

				278.28		1.003584

				278.3		1.003584

				278.32		1.003584

				278.34		1.003584

				278.36		1.003584

				278.38		1.003584

				278.4		1.003584

				278.43		1.003584

				278.45		1.003584

				278.47		1.003584

				278.49		1.003584

				278.51		1.003584

				278.53		1.003584

				278.55		1.003584

				278.57		1.003584

				278.59		1.003584

				278.61		1.003584

				278.64		1.009558

				278.66		1.009558

				278.68		1.009558

				278.7		1.009558

				278.72		1.009558

				278.74		1.009558

				278.76		1.009558

				278.78		1.009558

				278.8		1.009558

				278.82		1.009558

				278.85		1.009558

				278.87		1.009558

				278.89		1.009558

				278.91		1.009558

				278.93		1.009558

				278.95		1.009558

				278.97		1.009558

				278.99		1.015532

				279.01		1.015532

				279.03		1.015532

				279.06		1.015532

				279.08		1.015532

				279.1		1.015532

				279.12		1.015532

				279.14		1.015532

				279.16		1.015532

				279.18		1.021505

				279.2		1.021505

				279.22		1.021505

				279.24		1.021505

				279.27		1.021505

				279.29		1.021505

				279.31		1.027479

				279.33		1.027479

				279.35		1.027479

				279.37		1.027479

				279.39		1.027479

				279.41		1.027479

				279.43		1.027479

				279.45		1.027479

				279.48		1.027479

				279.5		1.027479

				279.52		1.027479

				279.54		1.027479

				279.56		1.027479

				279.58		1.027479

				279.6		1.027479

				279.62		1.027479

				279.64		1.027479

				279.66		1.027479

				279.69		1.027479

				279.71		1.027479

				279.73		1.027479

				279.75		1.027479

				279.77		1.027479

				279.79		1.027479

				279.81		1.027479

				279.83		1.027479

				279.85		1.027479

				279.87		1.027479

				279.89		1.027479

				279.92		1.027479

				279.94		1.027479

				279.96		1.033453

				279.98		1.027479

				280		1.027479

				280.02		1.033453

				280.04		1.033453

				280.06		1.033453

				280.08		1.033453

				280.1		1.033453

				280.13		1.033453

				280.15		1.033453

				280.17		1.033453

				280.19		1.033453

				280.21		1.033453

				280.23		1.033453

				280.25		1.033453

				280.27		1.033453

				280.29		1.033453

				280.31		1.033453

				280.34		1.033453

				280.36		1.033453

				280.38		1.033453

				280.4		1.033453

				280.42		1.033453

				280.44		1.039427

				280.46		1.039427

				280.48		1.039427

				280.5		1.039427

				280.52		1.039427

				280.54		1.039427

				280.57		1.039427

				280.59		1.039427

				280.61		1.039427

				280.63		1.039427

				280.65		1.039427

				280.67		1.039427

				280.69		1.039427

				280.71		1.039427

				280.73		1.039427

				280.75		1.039427

				280.78		1.033453

				280.8		1.039427

				280.82		1.033453

				280.84		1.033453

				280.86		1.033453

				280.88		1.033453

				280.9		1.033453

				280.92		1.033453

				280.94		1.033453

				280.96		1.033453

				280.99		1.033453

				281.01		1.033453

				281.03		1.033453

				281.05		1.033453

				281.07		1.033453

				281.09		1.033453

				281.11		1.033453

				281.13		1.033453

				281.15		1.033453

				281.17		1.033453

				281.2		1.033453

				281.22		1.033453

				281.24		1.033453

				281.26		1.033453

				281.28		1.033453

				281.3		1.033453

				281.32		1.033453

				281.34		1.033453

				281.36		1.033453

				281.38		1.033453

				281.4		1.033453

				281.43		1.033453

				281.45		1.033453

				281.47		1.033453

				281.49		1.033453

				281.51		1.033453

				281.53		1.027479

				281.55		1.027479

				281.57		1.027479

				281.59		1.027479

				281.61		1.027479

				281.64		1.033453

				281.66		1.027479

				281.68		1.027479

				281.7		1.033453

				281.72		1.033453

				281.74		1.033453

				281.76		1.033453

				281.78		1.033453

				281.8		1.033453

				281.82		1.033453

				281.85		1.033453

				281.87		1.033453

				281.89		1.033453

				281.91		1.033453

				281.93		1.033453

				281.95		1.033453

				281.97		1.033453

				281.99		1.033453

				282.01		1.033453

				282.03		1.033453

				282.06		1.033453

				282.08		1.033453

				282.1		1.033453

				282.12		1.033453

				282.14		1.033453

				282.16		1.033453

				282.18		1.033453

				282.2		1.033453

				282.22		1.033453

				282.24		1.033453

				282.27		1.033453

				282.29		1.033453

				282.31		1.033453

				282.33		1.033453

				282.35		1.033453

				282.37		1.033453

				282.39		1.033453

				282.41		1.033453

				282.43		1.033453

				282.45		1.033453

				282.48		1.033453

				282.5		1.033453

				282.52		1.033453

				282.54		1.033453

				282.56		1.033453

				282.58		1.033453

				282.6		1.033453

				282.62		1.033453

				282.64		1.033453

				282.66		1.033453

				282.69		1.033453

				282.71		1.033453

				282.73		1.033453

				282.75		1.033453

				282.77		1.033453

				282.79		1.033453

				282.81		1.033453

				282.83		1.033453

				282.85		1.033453

				282.87		1.033453

				282.9		1.033453

				282.92		1.033453

				282.94		1.033453

				282.96		1.033453

				282.98		1.027479

				283		1.027479

				283.02		1.033453

				283.04		1.033453

				283.06		1.027479

				283.08		1.027479

				283.11		1.027479

				283.13		1.027479

				283.15		1.027479

				283.17		1.027479

				283.19		1.027479

				283.21		1.027479

				283.23		1.027479

				283.25		1.027479

				283.27		1.027479

				283.29		1.027479

				283.32		1.033453

				283.34		1.033453

				283.36		1.027479

				283.38		1.027479

				283.4		1.033453

				283.42		1.027479

				283.44		1.033453

				283.46		1.033453

				283.48		1.033453

				283.5		1.033453

				283.53		1.033453

				283.55		1.033453

				283.57		1.033453

				283.59		1.033453

				283.61		1.033453

				283.63		1.033453

				283.65		1.033453

				283.67		1.033453

				283.69		1.033453

				283.72		1.033453

				283.74		1.033453

				283.76		1.033453

				283.78		1.033453

				283.8		1.033453

				283.82		1.033453

				283.84		1.033453

				283.86		1.033453

				283.88		1.033453

				283.9		1.033453

				283.93		1.033453

				283.95		1.033453

				283.97		1.033453

				283.99		1.033453

				284.01		1.033453

				284.03		1.033453

				284.05		1.033453

				284.07		1.033453

				284.09		1.033453

				284.11		1.033453

				284.14		1.033453

				284.16		1.033453

				284.18		1.033453

				284.2		1.033453

				284.22		1.033453

				284.24		1.033453

				284.26		1.033453

				284.28		1.033453

				284.3		1.033453

				284.32		1.033453

				284.35		1.033453

				284.37		1.033453

				284.39		1.033453

				284.41		1.033453

				284.43		1.039427

				284.45		1.033453

				284.47		1.033453

				284.49		1.033453

				284.51		1.033453

				284.53		1.033453

				284.56		1.033453

				284.58		1.033453

				284.6		1.033453

				284.62		1.033453

				284.64		1.033453

				284.66		1.033453

				284.68		1.033453

				284.7		1.033453

				284.72		1.033453

				284.74		1.033453

				284.77		1.033453

				284.79		1.033453

				284.81		1.033453

				284.83		1.033453

				284.85		1.033453

				284.87		1.033453

				284.89		1.033453

				284.91		1.033453

				284.93		1.033453

				284.95		1.033453

				284.98		1.033453

				285		1.033453

				285.02		1.033453

				285.04		1.033453

				285.06		1.033453

				285.08		1.033453

				285.1		1.033453

				285.12		1.033453

				285.14		1.033453

				285.16		1.033453

				285.19		1.033453

				285.21		1.033453

				285.23		1.033453

				285.25		1.033453

				285.27		1.027479

				285.29		1.027479

				285.31		1.033453

				285.33		1.027479

				285.35		1.027479

				285.37		1.027479

				285.4		1.027479

				285.42		1.027479

				285.44		1.027479

				285.46		1.027479

				285.48		1.027479

				285.5		1.033453

				285.52		1.027479

				285.54		1.027479

				285.56		1.027479

				285.58		1.027479

				285.61		1.027479

				285.63		1.027479

				285.65		1.027479

				285.67		1.027479

				285.69		1.027479

				285.71		1.027479

				285.73		1.027479

				285.75		1.027479

				285.77		1.027479

				285.8		1.027479

				285.82		1.027479

				285.84		1.027479

				285.86		1.027479

				285.88		1.027479

				285.9		1.027479

				285.92		1.027479

				285.94		1.027479

				285.96		1.021505

				285.98		1.021505

				286.01		1.021505

				286.03		1.021505

				286.05		1.021505

				286.07		1.021505

				286.09		1.021505

				286.11		1.021505

				286.13		1.021505

				286.15		1.021505

				286.17		1.021505

				286.19		1.021505

				286.22		1.021505

				286.24		1.015532

				286.26		1.021505

				286.28		1.015532

				286.3		1.015532

				286.32		1.015532

				286.34		1.021505

				286.36		1.021505

				286.38		1.021505

				286.4		1.021505

				286.43		1.021505

				286.45		1.021505

				286.47		1.021505

				286.49		1.021505

				286.51		1.015532

				286.53		1.015532

				286.55		1.015532

				286.57		1.015532

				286.59		1.015532

				286.61		1.015532

				286.64		1.015532

				286.66		1.015532

				286.68		1.015532

				286.7		1.015532

				286.72		1.015532

				286.74		1.015532

				286.76		1.015532

				286.78		1.015532

				286.8		1.015532

				286.82		1.015532

				286.85		1.015532

				286.87		1.015532

				286.89		1.015532

				286.91		1.015532

				286.93		1.015532

				286.95		1.015532

				286.97		1.015532

				286.99		1.009558

				287.01		1.015532

				287.03		1.009558

				287.06		1.009558

				287.08		1.015532

				287.1		1.009558

				287.12		1.009558

				287.14		1.009558

				287.16		1.009558

				287.18		1.009558

				287.2		1.009558

				287.22		1.009558

				287.24		1.009558

				287.27		1.009558

				287.29		1.009558

				287.31		1.009558

				287.33		1.009558

				287.35		1.009558

				287.37		1.009558

				287.39		1.009558

				287.41		1.009558

				287.43		1.009558

				287.45		1.009558

				287.48		1.009558

				287.5		1.009558

				287.52		1.009558

				287.54		1.009558

				287.56		1.009558

				287.58		1.009558

				287.6		1.009558

				287.62		1.009558

				287.64		1.009558

				287.66		1.009558

				287.69		1.015532

				287.71		1.015532

				287.73		1.009558

				287.75		1.009558

				287.77		1.009558

				287.79		1.009558

				287.81		1.009558

				287.83		1.009558

				287.85		1.009558

				287.88		1.009558

				287.9		1.009558

				287.92		1.009558

				287.94		1.009558

				287.96		1.009558

				287.98		1.009558

				288		1.009558

				288.02		1.009558

				288.04		1.009558

				288.06		1.009558

				288.08		1.009558

				288.11		1.009558

				288.13		1.009558

				288.15		1.009558

				288.17		1.009558

				288.19		1.009558

				288.21		1.009558

				288.23		1.009558

				288.25		1.009558

				288.27		1.009558

				288.3		1.009558

				288.32		1.009558

				288.34		1.009558

				288.36		1.009558

				288.38		1.009558

				288.4		1.009558

				288.42		1.009558

				288.44		1.009558

				288.46		1.009558

				288.48		1.009558

				288.51		1.009558

				288.53		1.009558

				288.55		1.009558

				288.57		1.009558

				288.59		1.009558

				288.61		1.009558

				288.63		1.009558

				288.65		1.015532

				288.67		1.015532

				288.69		1.015532

				288.72		1.009558

				288.74		1.009558

				288.76		1.009558

				288.78		1.015532

				288.8		1.015532

				288.82		1.015532

				288.84		1.009558

				288.86		1.009558

				288.88		1.015532

				288.9		1.015532

				288.93		1.015532

				288.95		1.015532

				288.97		1.015532

				288.99		1.015532

				289.01		1.015532

				289.03		1.015532

				289.05		1.015532

				289.07		1.015532

				289.09		1.015532

				289.11		1.015532

				289.14		1.015532

				289.16		1.015532

				289.18		1.015532

				289.2		1.015532

				289.22		1.015532

				289.24		1.015532

				289.26		1.015532

				289.28		1.015532

				289.3		1.015532

				289.32		1.015532

				289.35		1.015532

				289.37		1.015532

				289.39		1.015532

				289.41		1.015532

				289.43		1.015532

				289.45		1.015532

				289.47		1.015532

				289.49		1.015532

				289.51		1.015532

				289.54		1.015532

				289.56		1.015532

				289.58		1.015532

				289.6		1.015532

				289.62		1.015532

				289.64		1.015532

				289.66		1.015532

				289.68		1.015532

				289.7		1.015532

				289.72		1.015532

				289.75		1.015532

				289.77		1.015532

				289.79		1.015532

				289.81		1.015532

				289.83		1.015532

				289.85		1.015532

				289.87		1.015532

				289.89		1.015532

				289.91		1.015532

				289.93		1.015532

				289.96		1.015532

				289.98		1.015532

				290		1.015532

				290.02		1.015532

				290.04		1.015532

				290.06		1.015532

				290.08		1.015532

				290.1		1.015532

				290.12		1.015532

				290.14		1.015532

				290.17		1.015532

				290.19		1.015532

				290.21		1.015532

				290.23		1.021505

				290.25		1.015532

				290.27		1.021505

				290.29		1.021505

				290.31		1.021505

				290.33		1.021505

				290.35		1.021505

				290.38		1.021505

				290.4		1.021505

				290.42		1.021505

				290.44		1.021505

				290.46		1.021505

				290.48		1.021505

				290.5		1.021505

				290.52		1.021505

				290.54		1.021505

				290.56		1.021505

				290.59		1.021505

				290.61		1.021505

				290.63		1.021505

				290.65		1.021505

				290.67		1.021505

				290.69		1.021505

				290.71		1.021505

				290.73		1.021505

				290.75		1.021505

				290.78		1.021505

				290.8		1.021505

				290.82		1.021505

				290.84		1.021505

				290.86		1.021505

				290.88		1.021505

				290.9		1.021505

				290.92		1.027479

				290.94		1.021505

				290.96		1.021505

				290.99		1.021505

				291.01		1.021505

				291.03		1.021505

				291.05		1.021505

				291.07		1.021505

				291.09		1.021505

				291.11		1.021505

				291.13		1.021505

				291.15		1.021505

				291.17		1.021505

				291.2		1.021505

				291.22		1.021505

				291.24		1.021505

				291.26		1.021505

				291.28		1.021505

				291.3		1.021505

				291.32		1.021505

				291.34		1.021505

				291.36		1.021505

				291.38		1.021505

				291.41		1.021505

				291.43		1.021505

				291.45		1.021505

				291.47		1.021505

				291.49		1.021505

				291.51		1.021505

				291.53		1.027479

				291.55		1.021505

				291.57		1.027479

				291.6		1.027479

				291.62		1.027479

				291.64		1.027479

				291.66		1.027479

				291.68		1.027479

				291.7		1.027479

				291.72		1.027479

				291.74		1.027479

				291.76		1.027479

				291.78		1.027479

				291.81		1.027479

				291.83		1.027479

				291.85		1.027479

				291.87		1.027479

				291.89		1.027479

				291.91		1.027479

				291.93		1.027479

				291.95		1.027479

				291.97		1.027479

				291.99		1.027479

				292.02		1.027479

				292.04		1.027479

				292.06		1.027479

				292.08		1.027479

				292.1		1.027479

				292.12		1.027479

				292.14		1.027479

				292.16		1.027479

				292.18		1.027479

				292.2		1.027479

				292.23		1.027479

				292.25		1.027479

				292.27		1.027479

				292.29		1.027479

				292.31		1.027479

				292.33		1.027479

				292.35		1.027479

				292.37		1.027479

				292.39		1.027479

				292.41		1.027479

				292.44		1.027479

				292.46		1.027479

				292.48		1.021505

				292.5		1.021505

				292.52		1.021505

				292.54		1.021505

				292.56		1.021505

				292.58		1.021505

				292.6		1.021505

				292.62		1.021505

				292.65		1.021505

				292.67		1.021505

				292.69		1.021505

				292.71		1.021505

				292.73		1.021505

				292.75		1.021505

				292.77		1.021505

				292.79		1.021505

				292.81		1.021505

				292.84		1.021505

				292.86		1.021505

				292.88		1.021505

				292.9		1.021505

				292.92		1.021505

				292.94		1.021505

				292.96		1.021505

				292.98		1.021505

				293		1.015532

				293.02		1.015532

				293.05		1.015532

				293.07		1.015532

				293.09		1.015532

				293.11		1.015532

				293.13		1.015532

				293.15		1.015532

				293.17		1.015532

				293.19		1.015532

				293.21		1.015532

				293.23		1.015532

				293.26		1.015532

				293.28		1.015532

				293.3		1.015532

				293.32		1.015532

				293.34		1.015532

				293.36		1.015532

				293.38		1.015532

				293.4		1.015532

				293.42		1.015532

				293.45		1.015532

				293.47		1.015532

				293.49		1.015532

				293.51		1.015532

				293.53		1.015532

				293.55		1.015532

				293.57		1.015532

				293.59		1.015532

				293.61		1.015532

				293.63		1.015532

				293.66		1.015532

				293.68		1.015532

				293.7		1.015532

				293.72		1.015532

				293.74		1.015532

				293.76		1.015532

				293.78		1.015532

				293.8		1.015532

				293.82		1.015532

				293.84		1.015532

				293.87		1.015532

				293.89		1.015532

				293.91		1.015532

				293.93		1.015532

				293.95		1.015532

				293.97		1.015532

				293.99		1.015532

				294.01		1.009558

				294.03		1.009558

				294.06		1.015532

				294.08		1.015532

				294.1		1.015532

				294.12		1.015532

				294.14		1.015532

				294.16		1.015532

				294.18		1.015532

				294.2		1.015532

				294.22		1.015532

				294.24		1.015532

				294.27		1.015532

				294.29		1.015532

				294.31		1.015532

				294.33		1.015532

				294.35		1.015532

				294.37		1.015532

				294.39		1.015532

				294.41		1.015532

				294.43		1.015532

				294.45		1.015532

				294.48		1.015532

				294.5		1.015532

				294.52		1.015532

				294.54		1.015532

				294.56		1.015532

				294.58		1.015532

				294.6		1.015532

				294.62		1.015532

				294.64		1.015532

				294.67		1.015532

				294.69		1.015532

				294.71		1.015532

				294.73		1.015532

				294.75		1.015532

				294.77		1.015532

				294.79		1.015532

				294.81		1.015532

				294.83		1.015532

				294.85		1.015532

				294.88		1.015532

				294.9		1.015532

				294.92		1.015532

				294.94		1.015532

				294.96		1.015532

				294.98		1.015532

				295		1.015532

				295.02		1.015532

				295.04		1.015532

				295.07		1.015532

				295.09		1.015532

				295.11		1.015532

				295.13		1.015532

				295.15		1.015532

				295.17		1.021505

				295.19		1.015532

				295.21		1.021505

				295.23		1.021505

				295.25		1.021505

				295.28		1.021505

				295.3		1.021505

				295.32		1.015532

				295.34		1.015532

				295.36		1.021505

				295.38		1.021505

				295.4		1.015532

				295.42		1.015532

				295.44		1.015532

				295.47		1.015532

				295.49		1.015532

				295.51		1.015532

				295.53		1.015532

				295.55		1.015532

				295.57		1.015532

				295.59		1.015532

				295.61		1.015532

				295.63		1.015532

				295.65		1.015532

				295.68		1.015532

				295.7		1.015532

				295.72		1.015532

				295.74		1.015532

				295.76		1.015532

				295.78		1.015532

				295.8		1.015532

				295.82		1.015532

				295.84		1.015532

				295.87		1.015532

				295.89		1.009558

				295.91		1.009558

				295.93		1.009558

				295.95		1.015532

				295.97		1.015532

				295.99		1.015532

				296.01		1.015532

				296.03		1.015532

				296.05		1.015532

				296.08		1.015532

				296.1		1.015532

				296.12		1.015532

				296.14		1.015532

				296.16		1.015532

				296.18		1.015532

				296.2		1.015532

				296.22		1.015532

				296.24		1.015532

				296.27		1.015532

				296.29		1.015532

				296.31		1.015532

				296.33		1.015532

				296.35		1.015532

				296.37		1.009558

				296.39		1.009558

				296.41		1.009558

				296.43		1.009558

				296.45		1.015532

				296.48		1.015532

				296.5		1.009558

				296.52		1.009558

				296.54		1.009558

				296.56		1.009558

				296.58		1.009558

				296.6		1.015532

				296.62		1.009558

				296.64		1.009558

				296.66		1.009558

				296.69		1.009558

				296.71		1.009558

				296.73		1.009558

				296.75		1.009558

				296.77		1.009558

				296.79		1.009558

				296.81		1.009558

				296.83		1.009558

				296.85		1.009558

				296.88		1.009558

				296.9		1.009558

				296.92		1.009558

				296.94		1.009558

				296.96		1.009558

				296.98		1.009558

				297		1.009558

				297.02		1.009558

				297.04		1.009558

				297.07		1.003584

				297.09		1.003584

				297.11		1.003584

				297.13		1.003584

				297.15		1.003584

				297.17		1.003584

				297.19		1.003584

				297.21		1.003584

				297.23		1.003584

				297.25		1.003584

				297.28		1.003584

				297.3		1.003584

				297.32		1.003584

				297.34		0.9976105

				297.36		0.9976105

				297.38		1.003584

				297.4		0.9976105

				297.42		1.003584

				297.44		0.9976105

				297.47		0.9976105

				297.49		0.9976105

				297.51		0.9976105

				297.53		0.9976105

				297.55		0.9976105

				297.57		0.9976105

				297.59		0.9976105

				297.61		0.9976105

				297.63		0.9976105

				297.65		0.9976105

				297.68		0.9976105

				297.7		0.9976105

				297.72		0.9976105

				297.74		0.9976105

				297.76		0.9976105

				297.78		0.9976105

				297.8		0.9976105

				297.82		0.9976105

				297.84		0.9916368

				297.87		0.9916368

				297.89		0.9916368

				297.91		0.9916368

				297.93		0.9916368

				297.95		0.9916368

				297.97		0.9916368

				297.99		0.9916368

				298.01		0.9916368

				298.03		0.9916368

				298.05		0.9916368

				298.08		0.9916368

				298.1		0.9916368

				298.12		0.9916368

				298.14		0.9916368

				298.16		0.9916368

				298.18		0.9916368

				298.2		0.9856631

				298.22		0.9856631

				298.24		0.9856631

				298.27		0.9856631

				298.29		0.9856631

				298.31		0.9856631

				298.33		0.9856631

				298.35		0.9856631

				298.37		0.9856631

				298.39		0.9856631

				298.41		0.9856631

				298.43		0.9856631

				298.45		0.9856631

				298.48		0.9856631

				298.5		0.9856631

				298.52		0.9856631

				298.54		0.9796894

				298.56		0.9856631

				298.58		0.9796894

				298.6		0.9796894

				298.62		0.9796894

				298.64		0.9796894

				298.67		0.9796894

				298.69		0.9796894

				298.71		0.9796894

				298.73		0.9796894

				298.75		0.9796894

				298.77		0.9796894

				298.79		0.9796894

				298.81		0.9796894

				298.83		0.9796894

				298.85		0.9796894

				298.88		0.9796894

				298.9		0.9796894

				298.92		0.9796894

				298.94		0.9796894

				298.96		0.9796894

				298.98		0.9796894

				299		0.9796894

				299.02		0.9796894

				299.04		0.9796894

				299.07		0.9796894

				299.09		0.9796894

				299.11		0.9796894

				299.13		0.9796894

				299.15		0.9796894

				299.17		0.9796894

				299.19		0.9796894

				299.21		0.9796894

				299.23		0.9796894

				299.26		0.9796894

				299.28		0.9796894

				299.3		0.9796894

				299.32		0.9796894

				299.34		0.9796894

				299.36		0.9796894

				299.38		0.9796894

				299.4		0.9796894

				299.42		0.9796894

				299.44		0.9796894

				299.47		0.9796894

				299.49		0.9796894

				299.51		0.9796894

				299.53		0.9796894

				299.55		0.9796894

				299.57		0.9796894

				299.59		0.9796894

				299.61		0.9796894

				299.63		0.9796894

				299.66		0.9796894

				299.68		0.9796894

				299.7		0.9796894

				299.72		0.9796894

				299.74		0.9796894

				299.76		0.9796894

				299.78		0.9796894

				299.8		0.9796894

				299.82		0.9796894

				299.85		0.9796894

				299.87		0.9796894

				299.89		0.9796894

				299.91		0.9796894

				299.93		0.9796894

				299.95		0.9796894

				299.97		0.9796894

				299.99		0.9796894

				300.01		0.9796894

				300.03		0.9796894

				300.06		0.9796894

				300.08		0.9796894

				300.1		0.9796894

				300.12		0.9796894

				300.14		0.9796894

				300.16		0.9796894

				300.18		0.9796894

				300.2		0.9796894

				300.22		0.9796894

				300.25		0.9796894

				300.27		0.9796894

				300.29		0.9796894

				300.31		0.9796894

				300.33		0.9796894

				300.35		0.9796894

				300.37		0.9796894

				300.39		0.9796894

				300.41		0.9796894

				300.44		0.9796894

				300.46		0.9796894

				300.48		0.9796894

				300.5		0.9796894

				300.52		0.9796894

				300.54		0.9796894

				300.56		0.9796894

				300.58		0.9796894

				300.6		0.9737157

				300.62		0.9796894

				300.65		0.9737157

				300.67		0.9737157

				300.69		0.9796894

				300.71		0.9796894

				300.73		0.9796894

				300.75		0.9796894

				300.77		0.9796894

				300.79		0.9796894

				300.81		0.9737157

				300.84		0.9796894

				300.86		0.9796894

				300.88		0.9796894

				300.9		0.9796894

				300.92		0.9796894

				300.94		0.9737157

				300.96		0.9796894

				300.98		0.9737157

				301		0.9737157

				301.03		0.9737157

				301.05		0.9737157

				301.07		0.9737157

				301.09		0.9737157

				301.11		0.9737157

				301.13		0.9737157

				301.15		0.9737157

				301.17		0.9737157

				301.19		0.9737157

				301.21		0.9737157

				301.24		0.9737157

				301.26		0.9737157

				301.28		0.9737157

				301.3		0.9737157

				301.32		0.9737157

				301.34		0.9737157

				301.36		0.9737157

				301.38		0.9737157

				301.4		0.9737157

				301.43		0.9737157

				301.45		0.9737157

				301.47		0.9737157

				301.49		0.9737157

				301.51		0.9737157

				301.53		0.9737157

				301.55		0.9737157

				301.57		0.9737157

				301.59		0.9737157

				301.62		0.9737157

				301.64		0.9737157

				301.66		0.9737157

				301.68		0.9737157

				301.7		0.9737157

				301.72		0.9737157

				301.74		0.9737157

				301.76		0.9737157

				301.78		0.9737157

				301.8		0.9737157

				301.83		0.9737157

				301.85		0.9737157

				301.87		0.9737157

				301.89		0.9737157

				301.91		0.9737157

				301.93		0.9737157

				301.95		0.9737157

				301.97		0.9737157

				301.99		0.9737157

				302.02		0.9737157

				302.04		0.9737157

				302.06		0.9737157

				302.08		0.9737157

				302.1		0.9737157

				302.12		0.9737157

				302.14		0.9737157

				302.16		0.9737157

				302.18		0.9737157

				302.21		0.9737157

				302.23		0.9737157

				302.25		0.9737157

				302.27		0.9737157

				302.29		0.9737157

				302.31		0.9737157

				302.33		0.9737157

				302.35		0.9737157

				302.37		0.9737157

				302.39		0.9737157

				302.42		0.9737157

				302.44		0.9737157

				302.46		0.9737157

				302.48		0.9737157

				302.5		0.9737157

				302.52		0.9737157

				302.54		0.9737157

				302.56		0.9737157

				302.58		0.9737157

				302.61		0.9737157

				302.63		0.9737157

				302.65		0.9737157

				302.67		0.9737157

				302.69		0.9737157

				302.71		0.9737157

				302.73		0.9737157

				302.75		0.9737157

				302.77		0.9737157

				302.8		0.9737157

				302.82		0.9737157

				302.84		0.9737157

				302.86		0.9737157

				302.88		0.9737157

				302.9		0.9737157

				302.92		0.9737157

				302.94		0.9737157

				302.96		0.9737157

				302.99		0.9737157

				303.01		0.9737157

				303.03		0.9737157

				303.05		0.9737157

				303.07		0.9796894

				303.09		0.9796894

				303.11		0.9796894

				303.13		0.9796894

				303.15		0.9796894

				303.18		0.9796894

				303.2		0.9796894

				303.22		0.9796894

				303.24		0.9796894

				303.26		0.9796894

				303.28		0.9796894

				303.3		0.9796894

				303.32		0.9796894

				303.34		0.9796894

				303.36		0.9796894

				303.39		0.9796894

				303.41		0.9796894

				303.43		0.9796894

				303.45		0.9796894

				303.47		0.9796894

				303.49		0.9796894

				303.51		0.9856631

				303.53		0.9796894

				303.55		0.9796894

				303.58		0.9856631

				303.6		0.9856631

				303.62		0.9796894

				303.64		0.9856631

				303.66		0.9856631

				303.68		0.9856631

				303.7		0.9856631

				303.72		0.9856631

				303.74		0.9856631

				303.77		0.9856631

				303.79		0.9856631

				303.81		0.9856631

				303.83		0.9856631

				303.85		0.9856631

				303.87		0.9856631

				303.89		0.9856631

				303.91		0.9856631

				303.93		0.9856631

				303.96		0.9856631

				303.98		0.9856631

				304		0.9856631

				304.02		0.9856631

				304.04		0.9856631

				304.06		0.9856631

				304.08		0.9856631

				304.1		0.9856631

				304.12		0.9856631

				304.15		0.9856631

				304.17		0.9856631

				304.19		0.9856631

				304.21		0.9856631

				304.23		0.9856631

				304.25		0.9856631

				304.27		0.9856631

				304.29		0.9856631

				304.31		0.9856631

				304.33		0.9856631

				304.36		0.9856631

				304.38		0.9856631

				304.4		0.9856631

				304.42		0.9856631

				304.44		0.9856631

				304.46		0.9856631

				304.48		0.9856631

				304.5		0.9856631

				304.52		0.9856631

				304.55		0.9856631

				304.57		0.9856631

				304.59		0.9856631

				304.61		0.9856631

				304.63		0.9916368

				304.65		0.9916368

				304.67		0.9856631

				304.69		0.9916368

				304.71		0.9856631

				304.74		0.9916368

				304.76		0.9856631

				304.78		0.9916368

				304.8		0.9856631

				304.82		0.9856631

				304.84		0.9856631

				304.86		0.9856631

				304.88		0.9856631

				304.9		0.9856631

				304.93		0.9856631

				304.95		0.9856631

				304.97		0.9856631

				304.99		0.9856631

				305.01		0.9856631

				305.03		0.9856631

				305.05		0.9856631

				305.07		0.9856631

				305.09		0.9856631

				305.12		0.9856631

				305.14		0.9856631

				305.16		0.9856631

				305.18		0.9856631

				305.2		0.9856631

				305.22		0.9856631

				305.24		0.9856631

				305.26		0.9856631

				305.28		0.9856631

				305.3		0.9856631

				305.33		0.9856631

				305.35		0.9856631

				305.37		0.9856631

				305.39		0.9856631

				305.41		0.9856631

				305.43		0.9856631

				305.45		0.9856631

				305.47		0.9856631

				305.49		0.9796894

				305.52		0.9796894

				305.54		0.9796894

				305.56		0.9796894

				305.58		0.9796894

				305.6		0.9796894

				305.62		0.9796894

				305.64		0.9796894

				305.66		0.9796894

				305.68		0.9796894

				305.71		0.9796894

				305.73		0.9796894

				305.75		0.9796894

				305.77		0.9796894

				305.79		0.9796894

				305.81		0.9796894

				305.83		0.9796894

				305.85		0.9796894

				305.87		0.9796894

				305.89		0.9796894

				305.92		0.9796894

				305.94		0.9737157

				305.96		0.9796894

				305.98		0.9737157

				306		0.9737157

				306.02		0.9737157

				306.04		0.9737157

				306.06		0.9737157

				306.08		0.9737157

				306.11		0.9737157

				306.13		0.9737157

				306.15		0.9737157

				306.17		0.9737157

				306.19		0.9737157

				306.21		0.9737157

				306.23		0.9737157

				306.25		0.9737157

				306.27		0.9737157

				306.3		0.9737157

				306.32		0.9737157

				306.34		0.9737157

				306.36		0.9737157

				306.38		0.9737157

				306.4		0.9737157

				306.42		0.9737157

				306.44		0.9737157

				306.46		0.9737157

				306.49		0.9737157

				306.51		0.9737157

				306.53		0.9737157

				306.55		0.9737157

				306.57		0.9737157

				306.59		0.9737157

				306.61		0.9677419

				306.63		0.9677419

				306.65		0.9677419

				306.68		0.9677419

				306.7		0.9677419

				306.72		0.9677419

				306.74		0.9677419

				306.76		0.9677419

				306.78		0.9677419

				306.8		0.9677419

				306.82		0.9677419

				306.84		0.9677419

				306.87		0.9677419

				306.89		0.9677419

				306.91		0.9677419

				306.93		0.9677419

				306.95		0.9677419

				306.97		0.9677419

				306.99		0.9677419

				307.01		0.9677419

				307.03		0.9677419

				307.06		0.9677419

				307.08		0.9677419

				307.1		0.9677419

				307.12		0.9677419

				307.14		0.9677419

				307.16		0.9677419

				307.18		0.9677419

				307.2		0.9677419

				307.22		0.9617682

				307.25		0.9617682

				307.27		0.9617682

				307.29		0.9617682

				307.31		0.9617682

				307.33		0.9617682

				307.35		0.9617682

				307.37		0.9617682

				307.39		0.9617682

				307.41		0.9617682

				307.44		0.9617682

				307.46		0.9617682

				307.48		0.9617682

				307.5		0.9617682

				307.52		0.9617682

				307.54		0.9617682

				307.56		0.9557945

				307.58		0.9617682

				307.6		0.9617682

				307.63		0.9617682

				307.65		0.9617682

				307.67		0.9557945

				307.69		0.9617682

				307.71		0.9617682

				307.73		0.9557945

				307.75		0.9557945

				307.77		0.9557945

				307.79		0.9557945

				307.81		0.9557945

				307.84		0.9557945

				307.86		0.9557945

				307.88		0.9557945

				307.9		0.9557945

				307.92		0.9557945

				307.94		0.9557945

				307.96		0.9557945

				307.98		0.9557945

				308		0.9557945

				308.03		0.9557945

				308.05		0.9557945

				308.07		0.9557945

				308.09		0.9557945

				308.11		0.9557945

				308.13		0.9557945

				308.15		0.9557945

				308.17		0.9557945

				308.19		0.9557945

				308.22		0.9557945

				308.24		0.9557945

				308.26		0.9557945

				308.28		0.9557945

				308.3		0.9557945

				308.32		0.9557945

				308.34		0.9557945

				308.36		0.9557945

				308.38		0.9557945

				308.41		0.9557945

				308.43		0.9557945

				308.45		0.9557945

				308.47		0.9557945

				308.49		0.9557945

				308.51		0.9557945

				308.53		0.9557945

				308.55		0.9557945

				308.57		0.9557945

				308.6		0.9557945

				308.62		0.9557945

				308.64		0.9557945

				308.66		0.9557945

				308.68		0.9557945

				308.7		0.9557945

				308.72		0.9557945

				308.74		0.9557945

				308.76		0.9557945

				308.79		0.9557945

				308.81		0.9557945

				308.83		0.9557945

				308.85		0.9557945

				308.87		0.9557945

				308.89		0.9557945

				308.91		0.9557945

				308.93		0.9557945

				308.95		0.9557945

				308.97		0.9557945

				309		0.9557945

				309.02		0.9557945

				309.04		0.9557945

				309.06		0.9557945

				309.08		0.9557945

				309.1		0.9557945

				309.12		0.9557945

				309.14		0.9557945

				309.16		0.9557945

				309.19		0.9557945

				309.21		0.9557945

				309.23		0.9557945

				309.25		0.9557945

				309.27		0.9557945

				309.29		0.9557945

				309.31		0.9557945

				309.33		0.9557945

				309.35		0.9557945

				309.38		0.9557945

				309.4		0.9557945

				309.42		0.9557945

				309.44		0.9557945

				309.46		0.9557945

				309.48		0.9557945

				309.5		0.9557945

				309.52		0.9557945

				309.54		0.9557945

				309.57		0.9557945

				309.59		0.9557945

				309.61		0.9557945

				309.63		0.9557945

				309.65		0.9617682

				309.67		0.9557945

				309.69		0.9617682

				309.71		0.9557945

				309.73		0.9617682

				309.76		0.9617682

				309.78		0.9557945

				309.8		0.9617682

				309.82		0.9617682

				309.84		0.9617682

				309.86		0.9617682

				309.88		0.9617682

				309.9		0.9617682

				309.92		0.9617682

				309.95		0.9617682

				309.97		0.9617682

				309.99		0.9617682

				310.01		0.9617682

				310.03		0.9617682

				310.05		0.9617682

				310.07		0.9617682

				310.09		0.9617682

				310.11		0.9617682

				310.14		0.9617682

				310.16		0.9617682

				310.18		0.9617682

				310.2		0.9617682

				310.22		0.9617682

				310.24		0.9617682

				310.26		0.9617682

				310.28		0.9617682

				310.3		0.9617682

				310.33		0.9617682

				310.35		0.9617682

				310.37		0.9617682

				310.39		0.9617682

				310.41		0.9617682

				310.43		0.9677419

				310.45		0.9677419

				310.47		0.9677419

				310.49		0.9617682

				310.52		0.9677419

				310.54		0.9677419

				310.56		0.9617682

				310.58		0.9617682

				310.6		0.9617682

				310.62		0.9677419

				310.64		0.9677419

				310.66		0.9677419

				310.68		0.9677419

				310.71		0.9677419

				310.73		0.9677419

				310.75		0.9677419

				310.77		0.9677419

				310.79		0.9677419

				310.81		0.9677419

				310.83		0.9677419

				310.85		0.9677419

				310.87		0.9677419

				310.9		0.9677419

				310.92		0.9677419

				310.94		0.9677419

				310.96		0.9677419

				310.98		0.9677419

				311		0.9677419

				311.02		0.9677419

				311.04		0.9677419

				311.06		0.9737157

				311.09		0.9737157

				311.11		0.9737157

				311.13		0.9737157

				311.15		0.9737157

				311.17		0.9737157

				311.19		0.9737157

				311.21		0.9737157

				311.23		0.9737157

				311.25		0.9737157

				311.28		0.9737157

				311.3		0.9737157

				311.32		0.9737157

				311.34		0.9737157

				311.36		0.9737157

				311.38		0.9737157

				311.4		0.9737157

				311.42		0.9737157

				311.44		0.9737157

				311.47		0.9737157

				311.49		0.9737157

				311.51		0.9737157

				311.53		0.9737157

				311.55		0.9737157

				311.57		0.9737157

				311.59		0.9737157

				311.61		0.9737157

				311.63		0.9737157

				311.65		0.9737157

				311.68		0.9737157

				311.7		0.9737157

				311.72		0.9737157

				311.74		0.9737157

				311.76		0.9737157

				311.78		0.9737157

				311.8		0.9737157

				311.82		0.9737157

				311.84		0.9737157

				311.87		0.9737157

				311.89		0.9737157

				311.91		0.9737157

				311.93		0.9737157

				311.95		0.9737157

				311.97		0.9737157

				311.99		0.9737157

				312.01		0.9737157

				312.03		0.9737157

				312.06		0.9737157

				312.08		0.9737157

				312.1		0.9737157

				312.12		0.9737157

				312.14		0.9677419

				312.16		0.9737157

				312.18		0.9737157

				312.2		0.9737157

				312.22		0.9737157

				312.25		0.9737157

				312.27		0.9737157

				312.29		0.9737157

				312.31		0.9737157

				312.33		0.9737157

				312.35		0.9737157

				312.37		0.9737157

				312.39		0.9737157

				312.41		0.9737157

				312.44		0.9737157

				312.46		0.9677419

				312.48		0.9677419

				312.5		0.9677419

				312.52		0.9677419

				312.54		0.9677419

				312.56		0.9677419

				312.58		0.9677419

				312.6		0.9677419

				312.63		0.9677419

				312.65		0.9677419

				312.67		0.9677419

				312.69		0.9677419

				312.71		0.9677419

				312.73		0.9677419

				312.75		0.9677419

				312.77		0.9677419

				312.79		0.9677419

				312.82		0.9677419

				312.84		0.9677419

				312.86		0.9677419

				312.88		0.9677419

				312.9		0.9677419

				312.92		0.9677419

				312.94		0.9677419

				312.96		0.9677419

				312.98		0.9677419

				313.01		0.9677419

				313.03		0.9617682

				313.05		0.9617682

				313.07		0.9617682

				313.09		0.9617682

				313.11		0.9617682

				313.13		0.9617682

				313.15		0.9617682

				313.17		0.9617682

				313.2		0.9617682

				313.22		0.9617682

				313.24		0.9617682

				313.26		0.9617682

				313.28		0.9617682

				313.3		0.9617682

				313.32		0.9617682

				313.34		0.9617682

				313.37		0.9617682

				313.39		0.9617682

				313.41		0.9617682

				313.43		0.9617682

				313.45		0.9557945

				313.47		0.9557945

				313.49		0.9617682

				313.51		0.9617682

				313.53		0.9617682

				313.56		0.9617682

				313.58		0.9617682

				313.6		0.9617682

				313.62		0.9617682

				313.64		0.9617682

				313.66		0.9617682

				313.68		0.9617682

				313.7		0.9617682

				313.72		0.9617682

				313.75		0.9617682

				313.77		0.9617682

				313.79		0.9617682

				313.81		0.9617682

				313.83		0.9617682

				313.85		0.9617682

				313.87		0.9617682

				313.89		0.9617682

				313.91		0.9617682

				313.94		0.9617682

				313.96		0.9617682

				313.98		0.9617682

				314		0.9617682

				314.02		0.9617682

				314.04		0.9617682

				314.06		0.9617682

				314.08		0.9617682

				314.1		0.9617682

				314.13		0.9617682

				314.15		0.9617682

				314.17		0.9617682

				314.19		0.9617682

				314.21		0.9617682

				314.23		0.9617682

				314.25		0.9617682

				314.27		0.9617682

				314.3		0.9617682

				314.32		0.9617682

				314.34		0.9617682

				314.36		0.9617682

				314.38		0.9557945

				314.4		0.9557945

				314.42		0.9557945

				314.44		0.9557945

				314.46		0.9557945

				314.49		0.9557945

				314.51		0.9557945

				314.53		0.9557945

				314.55		0.9557945

				314.57		0.9557945

				314.59		0.9557945

				314.61		0.9557945

				314.63		0.9557945

				314.65		0.9557945

				314.68		0.9557945

				314.7		0.9557945

				314.72		0.9557945

				314.74		0.9557945

				314.76		0.9557945

				314.78		0.9557945

				314.8		0.9557945

				314.82		0.9557945

				314.84		0.9557945

				314.87		0.9557945

				314.89		0.9557945

				314.91		0.9557945

				314.93		0.9557945

				314.95		0.9557945

				314.97		0.9557945

				314.99		0.9557945

				315.01		0.9557945

				315.03		0.9498208

				315.06		0.9557945

				315.08		0.9557945

				315.1		0.9557945

				315.12		0.9557945

				315.14		0.9557945

				315.16		0.9557945

				315.18		0.9557945

				315.2		0.9557945

				315.22		0.9557945

				315.25		0.9557945

				315.27		0.9557945

				315.29		0.9557945

				315.31		0.9557945

				315.33		0.9557945

				315.35		0.9557945

				315.37		0.9557945

				315.39		0.9557945

				315.42		0.9557945

				315.44		0.9557945

				315.46		0.9557945

				315.48		0.9557945

				315.5		0.9557945

				315.52		0.9557945

				315.54		0.9557945

				315.56		0.9557945

				315.58		0.9498208

				315.61		0.9498208

				315.63		0.9498208

				315.65		0.9498208

				315.67		0.9498208

				315.69		0.9498208

				315.71		0.9498208

				315.73		0.9498208

				315.75		0.9498208

				315.78		0.9498208

				315.8		0.9498208

				315.82		0.9498208

				315.84		0.9498208

				315.86		0.9498208

				315.88		0.9498208

				315.9		0.9498208

				315.92		0.9438471

				315.94		0.9438471

				315.97		0.9438471

				315.99		0.9438471

				316.01		0.9498208

				316.03		0.9438471

				316.05		0.9438471

				316.07		0.9438471

				316.09		0.9438471

				316.11		0.9438471

				316.14		0.9438471

				316.16		0.9438471

				316.18		0.9438471

				316.2		0.9438471

				316.22		0.9438471

				316.24		0.9438471

				316.26		0.9438471

				316.28		0.9438471

				316.3		0.9498208

				316.33		0.9438471

				316.35		0.9438471

				316.37		0.9438471

				316.39		0.9498208

				316.41		0.9438471

				316.43		0.9438471

				316.45		0.9438471

				316.47		0.9438471

				316.5		0.9498208

				316.52		0.9498208

				316.54		0.9498208

				316.56		0.9498208

				316.58		0.9498208

				316.6		0.9498208

				316.62		0.9498208

				316.64		0.9498208

				316.66		0.9438471

				316.69		0.9498208

				316.71		0.9498208

				316.73		0.9498208

				316.75		0.9498208

				316.77		0.9438471

				316.79		0.9438471

				316.81		0.9498208

				316.83		0.9438471

				316.85		0.9438471

				316.88		0.9438471

				316.9		0.9498208

				316.92		0.9498208

				316.94		0.9498208

				316.96		0.9498208

				316.98		0.9438471

				317		0.9438471

				317.02		0.9438471

				317.05		0.9438471

				317.07		0.9438471

				317.09		0.9438471

				317.11		0.9438471

				317.13		0.9438471

				317.15		0.9438471

				317.17		0.9438471

				317.19		0.9438471

				317.21		0.9438471

				317.24		0.9438471

				317.26		0.9438471

				317.28		0.9438471

				317.3		0.9438471

				317.32		0.9438471

				317.34		0.9438471

				317.36		0.9438471

				317.38		0.9438471

				317.41		0.9438471

				317.43		0.9378734

				317.45		0.9438471

				317.47		0.9438471

				317.49		0.9438471

				317.51		0.9378734

				317.53		0.9378734

				317.55		0.9378734

				317.57		0.9378734

				317.6		0.9378734

				317.62		0.9378734

				317.64		0.9378734

				317.66		0.9378734

				317.68		0.9378734

				317.7		0.9378734

				317.72		0.9378734

				317.74		0.9378734

				317.77		0.9378734

				317.79		0.9378734

				317.81		0.9378734

				317.83		0.9378734

				317.85		0.9378734

				317.87		0.9378734

				317.89		0.9378734

				317.91		0.9378734

				317.93		0.9378734

				317.96		0.9378734

				317.98		0.9378734

				318		0.9378734

				318.02		0.9378734

				318.04		0.9378734

				318.06		0.9378734

				318.08		0.9378734

				318.1		0.9378734

				318.13		0.9378734

				318.15		0.9318996

				318.17		0.9318996

				318.19		0.9318996

				318.21		0.9318996

				318.23		0.9318996

				318.25		0.9318996

				318.27		0.9318996

				318.29		0.9318996

				318.32		0.9318996

				318.34		0.9318996

				318.36		0.9318996

				318.38		0.9318996

				318.4		0.9318996

				318.42		0.9318996

				318.44		0.9318996

				318.46		0.9318996

				318.49		0.9318996

				318.51		0.9318996

				318.53		0.9318996

				318.55		0.9318996

				318.57		0.9318996

				318.59		0.9318996

				318.61		0.9318996

				318.63		0.9318996

				318.65		0.9318996

				318.68		0.9318996

				318.7		0.9259259

				318.72		0.9259259

				318.74		0.9259259

				318.76		0.9259259

				318.78		0.9259259

				318.8		0.9259259

				318.82		0.9259259

				318.84		0.9259259

				318.87		0.9259259

				318.89		0.9259259

				318.91		0.9259259

				318.93		0.9259259

				318.95		0.9259259

				318.97		0.9259259

				318.99		0.9259259

				319.01		0.9259259

				319.04		0.9259259

				319.06		0.9259259

				319.08		0.9259259

				319.1		0.9259259

				319.12		0.9259259

				319.14		0.9259259

				319.16		0.9259259

				319.18		0.9259259

				319.2		0.9259259

				319.23		0.9259259

				319.25		0.9259259

				319.27		0.9259259

				319.29		0.9259259

				319.31		0.9259259

				319.33		0.9259259

				319.35		0.9259259

				319.37		0.9259259

				319.4		0.9259259

				319.42		0.9259259

				319.44		0.9259259

				319.46		0.9259259

				319.48		0.9259259

				319.5		0.9199522

				319.52		0.9199522

				319.54		0.9199522

				319.57		0.9199522

				319.59		0.9199522

				319.61		0.9199522

				319.63		0.9199522

				319.65		0.9199522

				319.67		0.9199522

				319.69		0.9199522

				319.71		0.9199522

				319.73		0.9199522

				319.76		0.9199522

				319.78		0.9199522

				319.8		0.9199522

				319.82		0.9199522

				319.84		0.9199522

				319.86		0.9199522

				319.88		0.9199522

				319.9		0.9199522

				319.93		0.9199522

				319.95		0.9199522

				319.97		0.9199522

				319.99		0.9199522

				320.01		0.9199522

				320.03		0.9199522

				320.05		0.9199522

				320.07		0.9199522

				320.09		0.9199522

				320.12		0.9199522

				320.14		0.9199522

				320.16		0.9199522

				320.18		0.9199522

				320.2		0.9199522

				320.22		0.9199522

				320.24		0.9199522

				320.26		0.9199522

				320.29		0.9199522

				320.31		0.9199522

				320.33		0.9199522

				320.35		0.9199522

				320.37		0.9199522

				320.39		0.9199522

				320.41		0.9199522

				320.43		0.9199522

				320.45		0.9199522

				320.48		0.9139785

				320.5		0.9139785

				320.52		0.9199522

				320.54		0.9139785

				320.56		0.9139785

				320.58		0.9139785

				320.6		0.9139785

				320.62		0.9139785

				320.65		0.9139785

				320.67		0.9139785

				320.69		0.9139785

				320.71		0.9139785

				320.73		0.9139785

				320.75		0.9139785

				320.77		0.9139785

				320.79		0.9139785

				320.81		0.9139785

				320.84		0.9139785

				320.86		0.9139785

				320.88		0.9139785

				320.9		0.9139785

				320.92		0.9139785

				320.94		0.9139785

				320.96		0.9139785

				320.98		0.9139785

				321.01		0.9139785

				321.03		0.9139785

				321.05		0.9139785

				321.07		0.9139785

				321.09		0.9139785

				321.11		0.9139785

				321.13		0.9139785

				321.15		0.9139785

				321.17		0.9139785

				321.2		0.9139785

				321.22		0.9139785

				321.24		0.9139785

				321.26		0.9139785

				321.28		0.9139785

				321.3		0.9139785

				321.32		0.9139785

				321.34		0.9139785

				321.37		0.9139785

				321.39		0.9139785

				321.41		0.9139785

				321.43		0.9139785

				321.45		0.9139785

				321.47		0.9139785

				321.49		0.9139785

				321.51		0.9139785

				321.53		0.9139785

				321.56		0.9139785

				321.58		0.9139785

				321.6		0.9139785

				321.62		0.9139785

				321.64		0.9139785

				321.66		0.9139785

				321.68		0.9139785

				321.7		0.9139785

				321.72		0.9199522

				321.75		0.9139785

				321.77		0.9199522

				321.79		0.9199522

				321.81		0.9199522

				321.83		0.9199522

				321.85		0.9199522

				321.87		0.9199522

				321.89		0.9199522

				321.92		0.9199522

				321.94		0.9199522

				321.96		0.9199522

				321.98		0.9199522

				322		0.9199522

				322.02		0.9199522

				322.04		0.9199522

				322.06		0.9199522

				322.08		0.9199522

				322.11		0.9199522

				322.13		0.9199522

				322.15		0.9199522

				322.17		0.9199522

				322.19		0.9199522

				322.21		0.9199522

				322.23		0.9199522

				322.25		0.9199522

				322.28		0.9199522

				322.3		0.9199522

				322.32		0.9199522

				322.34		0.9199522

				322.36		0.9199522

				322.38		0.9199522

				322.4		0.9199522

				322.42		0.9199522

				322.44		0.9259259

				322.47		0.9259259

				322.49		0.9259259

				322.51		0.9259259

				322.53		0.9259259

				322.55		0.9259259

				322.57		0.9259259

				322.59		0.9259259

				322.61		0.9259259

				322.64		0.9259259

				322.66		0.9259259

				322.68		0.9259259

				322.7		0.9259259

				322.72		0.9259259

				322.74		0.9318996

				322.76		0.9318996

				322.78		0.9318996

				322.8		0.9318996

				322.83		0.9318996

				322.85		0.9318996

				322.87		0.9318996

				322.89		0.9318996

				322.91		0.9318996

				322.93		0.9318996

				322.95		0.9318996

				322.97		0.9318996

				323		0.9318996

				323.02		0.9318996

				323.04		0.9318996

				323.06		0.9318996

				323.08		0.9318996

				323.1		0.9318996

				323.12		0.9318996

				323.14		0.9318996

				323.16		0.9318996

				323.19		0.9318996

				323.21		0.9318996

				323.23		0.9318996

				323.25		0.9318996

				323.27		0.9318996

				323.29		0.9318996

				323.31		0.9318996

				323.33		0.9318996

				323.35		0.9318996

				323.38		0.9318996

				323.4		0.9318996

				323.42		0.9318996

				323.44		0.9318996

				323.46		0.9318996

				323.48		0.9318996

				323.5		0.9318996

				323.52		0.9318996

				323.55		0.9318996

				323.57		0.9318996

				323.59		0.9318996

				323.61		0.9318996

				323.63		0.9318996

				323.65		0.9318996

				323.67		0.9318996

				323.69		0.9318996

				323.71		0.9318996

				323.74		0.9318996

				323.76		0.9318996

				323.78		0.9318996

				323.8		0.9318996

				323.82		0.9318996

				323.84		0.9318996

				323.86		0.9318996

				323.88		0.9318996

				323.91		0.9318996

				323.93		0.9318996

				323.95		0.9318996

				323.97		0.9318996

				323.99		0.9318996

				324.01		0.9318996

				324.03		0.9318996

				324.05		0.9318996

				324.07		0.9318996

				324.1		0.9318996

				324.12		0.9318996

				324.14		0.9318996

				324.16		0.9318996

				324.18		0.9318996

				324.2		0.9318996

				324.22		0.9318996

				324.24		0.9318996

				324.27		0.9318996

				324.29		0.9318996

				324.31		0.9318996

				324.33		0.9318996

				324.35		0.9318996

				324.37		0.9318996

				324.39		0.9318996

				324.41		0.9318996

				324.43		0.9318996

				324.46		0.9318996

				324.48		0.9318996

				324.5		0.9318996

				324.52		0.9318996

				324.54		0.9318996

				324.56		0.9318996

				324.58		0.9259259

				324.6		0.9259259

				324.63		0.9318996

				324.65		0.9259259

				324.67		0.9259259

				324.69		0.9259259

				324.71		0.9259259

				324.73		0.9259259

				324.75		0.9259259

				324.77		0.9259259

				324.79		0.9259259

				324.82		0.9259259

				324.84		0.9259259

				324.86		0.9259259

				324.88		0.9259259

				324.9		0.9259259

				324.92		0.9259259

				324.94		0.9259259

				324.96		0.9199522

				324.99		0.9259259

				325.01		0.9199522

				325.03		0.9199522

				325.05		0.9259259

				325.07		0.9199522

				325.09		0.9199522

				325.11		0.9199522

				325.13		0.9199522

				325.15		0.9199522

				325.18		0.9199522

				325.2		0.9199522

				325.22		0.9199522

				325.24		0.9199522

				325.26		0.9199522

				325.28		0.9199522

				325.3		0.9199522

				325.32		0.9199522

				325.35		0.9199522

				325.37		0.9199522

				325.39		0.9199522

				325.41		0.9199522

				325.43		0.9199522

				325.45		0.9199522

				325.47		0.9199522

				325.49		0.9199522

				325.52		0.9199522

				325.54		0.9199522

				325.56		0.9199522

				325.58		0.9199522

				325.6		0.9199522

				325.62		0.9199522

				325.64		0.9199522

				325.66		0.9199522

				325.68		0.9199522

				325.71		0.9199522

				325.73		0.9199522

				325.75		0.9199522

				325.77		0.9199522

				325.79		0.9199522

				325.81		0.9139785

				325.83		0.9199522

				325.85		0.9199522

				325.88		0.9139785

				325.9		0.9139785

				325.92		0.9139785

				325.94		0.9139785

				325.96		0.9139785

				325.98		0.9139785

				326		0.9139785

				326.02		0.9139785

				326.05		0.9139785

				326.07		0.9139785

				326.09		0.9139785

				326.11		0.9139785

				326.13		0.9139785

				326.15		0.9139785

				326.17		0.9139785

				326.19		0.9139785

				326.21		0.9139785

				326.24		0.9139785

				326.26		0.9139785

				326.28		0.9139785

				326.3		0.9080048

				326.32		0.9080048

				326.34		0.9139785

				326.36		0.9080048

				326.38		0.9080048

				326.41		0.9139785

				326.43		0.9080048

				326.45		0.9080048

				326.47		0.9080048

				326.49		0.9080048

				326.51		0.9080048

				326.53		0.9080048

				326.55		0.9080048

				326.58		0.9080048

				326.6		0.9080048

				326.62		0.9080048

				326.64		0.9080048

				326.66		0.9080048

				326.68		0.9080048

				326.7		0.9080048

				326.72		0.9080048

				326.74		0.9080048

				326.77		0.9080048

				326.79		0.9080048

				326.81		0.9080048

				326.83		0.9080048

				326.85		0.9080048

				326.87		0.9080048

				326.89		0.9080048

				326.91		0.9080048

				326.94		0.9080048

				326.96		0.9080048

				326.98		0.9080048

				327		0.9080048

				327.02		0.9080048

				327.04		0.9080048

				327.06		0.9080048

				327.08		0.9080048

				327.11		0.9080048

				327.13		0.9080048

				327.15		0.9020311

				327.17		0.9020311

				327.19		0.9020311

				327.21		0.9020311

				327.23		0.9020311

				327.25		0.9020311

				327.27		0.9020311

				327.3		0.9020311

				327.32		0.9020311

				327.34		0.9020311

				327.36		0.9020311

				327.38		0.9020311

				327.4		0.9020311

				327.42		0.9020311

				327.44		0.9020311

				327.46		0.9020311

				327.49		0.9020311

				327.51		0.9020311

				327.53		0.9020311

				327.55		0.9020311

				327.57		0.9020311

				327.59		0.9020311

				327.61		0.9020311

				327.63		0.9020311

				327.66		0.9020311

				327.68		0.9020311

				327.7		0.9020311

				327.72		0.9020311

				327.74		0.9020311

				327.76		0.9020311

				327.78		0.9020311

				327.8		0.9020311

				327.82		0.9020311

				327.85		0.9020311

				327.87		0.9020311

				327.89		0.9020311

				327.91		0.9020311

				327.93		0.9020311

				327.95		0.9020311

				327.97		0.9020311

				327.99		0.9020311

				328.02		0.9020311

				328.04		0.9020311

				328.06		0.9020311

				328.08		0.9020311

				328.1		0.9020311

				328.12		0.9020311

				328.14		0.9020311

				328.16		0.9020311

				328.18		0.9020311

				328.21		0.9020311

				328.23		0.9020311

				328.25		0.9020311

				328.27		0.9020311

				328.29		0.8960573

				328.31		0.8960573

				328.33		0.8960573

				328.35		0.9020311

				328.38		0.9020311

				328.4		0.9020311

				328.42		0.9020311

				328.44		0.9020311

				328.46		0.9020311

				328.48		0.9020311

				328.5		0.9020311

				328.52		0.9020311

				328.54		0.8960573

				328.57		0.9020311

				328.59		0.9020311

				328.61		0.8960573

				328.63		0.9020311

				328.65		0.8960573

				328.67		0.8960573

				328.69		0.9020311

				328.71		0.9020311

				328.73		0.9020311

				328.76		0.9020311

				328.78		0.8960573

				328.8		0.8960573

				328.82		0.8960573

				328.84		0.8960573

				328.86		0.8960573

				328.88		0.8960573

				328.9		0.8960573

				328.93		0.8960573

				328.95		0.8960573

				328.97		0.8960573

				328.99		0.8960573

				329.01		0.8960573

				329.03		0.8960573

				329.05		0.8960573

				329.07		0.8960573

				329.09		0.8960573

				329.12		0.8960573

				329.14		0.8960573

				329.16		0.8960573

				329.18		0.8960573

				329.2		0.8960573

				329.22		0.9020311

				329.24		0.8960573

				329.26		0.8960573

				329.29		0.8960573

				329.31		0.8960573

				329.33		0.8960573

				329.35		0.8960573

				329.37		0.8960573

				329.39		0.8960573

				329.41		0.8960573

				329.43		0.8960573

				329.45		0.8960573

				329.48		0.8960573

				329.5		0.8960573

				329.52		0.8960573

				329.54		0.8960573

				329.56		0.8960573

				329.58		0.8960573

				329.6		0.8960573

				329.62		0.8960573

				329.65		0.9020311

				329.67		0.8960573

				329.69		0.8960573

				329.71		0.8960573

				329.73		0.8960573

				329.75		0.8960573

				329.77		0.8960573

				329.79		0.8960573

				329.81		0.8960573

				329.84		0.8960573

				329.86		0.8960573

				329.88		0.8960573

				329.9		0.8960573

				329.92		0.8960573

				329.94		0.8960573

				329.96		0.8960573

				329.98		0.8960573

				330		0.8960573

				330.03		0.8960573

				330.05		0.8960573

				330.07		0.8960573

				330.09		0.8960573

				330.11		0.8960573

				330.13		0.8960573

				330.15		0.8960573

				330.17		0.8960573

				330.2		0.8960573

				330.22		0.8960573

				330.24		0.9020311

				330.26		0.9020311

				330.28		0.9020311

				330.3		0.9020311

				330.32		0.9020311

				330.34		0.9020311

				330.36		0.9020311

				330.39		0.9020311

				330.41		0.9020311

				330.43		0.9020311

				330.45		0.9020311

				330.47		0.9020311

				330.49		0.9020311

				330.51		0.9020311

				330.53		0.9020311

				330.55		0.9020311

				330.58		0.9020311

				330.6		0.9020311

				330.62		0.9020311

				330.64		0.9020311

				330.66		0.9020311

				330.68		0.9020311

				330.7		0.9020311

				330.72		0.9020311

				330.75		0.9020311

				330.77		0.9020311

				330.79		0.9020311

				330.81		0.9020311

				330.83		0.9020311

				330.85		0.9020311

				330.87		0.9020311

				330.89		0.9020311

				330.91		0.9020311

				330.94		0.9020311

				330.96		0.8960573

				330.98		0.9020311

				331		0.9080048

				331.02		0.9020311

				331.04		0.9020311

				331.06		0.9080048

				331.08		0.9080048

				331.1		0.9080048

				331.13		0.9080048

				331.15		0.9080048

				331.17		0.9080048

				331.19		0.9080048

				331.21		0.9080048

				331.23		0.9080048

				331.25		0.9080048

				331.27		0.9080048

				331.3		0.9080048

				331.32		0.9080048

				331.34		0.9080048

				331.36		0.9080048

				331.38		0.9080048

				331.4		0.9080048

				331.42		0.9080048

				331.44		0.9080048

				331.46		0.9080048

				331.49		0.9080048

				331.51		0.9080048

				331.53		0.9080048

				331.55		0.9080048

				331.57		0.9080048

				331.59		0.9080048

				331.61		0.9080048

				331.63		0.9080048

				331.65		0.9080048

				331.68		0.9080048

				331.7		0.9080048

				331.72		0.9080048

				331.74		0.9080048

				331.76		0.9080048

				331.78		0.9020311

				331.8		0.9080048

				331.82		0.9020311

				331.84		0.9080048

				331.87		0.9080048

				331.89		0.9080048

				331.91		0.9080048

				331.93		0.9020311

				331.95		0.9020311

				331.97		0.9020311

				331.99		0.9020311

				332.01		0.9020311

				332.03		0.9020311

				332.06		0.9020311

				332.08		0.9020311

				332.1		0.9020311

				332.12		0.9020311

				332.14		0.9020311

				332.16		0.9020311

				332.18		0.9020311

				332.2		0.9020311

				332.23		0.9020311

				332.25		0.9020311

				332.27		0.9020311

				332.29		0.9020311

				332.31		0.9020311

				332.33		0.9020311

				332.35		0.9020311

				332.37		0.9020311

				332.39		0.9020311

				332.42		0.9020311

				332.44		0.9020311

				332.46		0.9020311

				332.48		0.9020311

				332.5		0.9020311

				332.52		0.9020311

				332.54		0.9020311

				332.56		0.9020311

				332.58		0.9080048

				332.61		0.9020311

				332.63		0.9020311

				332.65		0.9020311

				332.67		0.9020311

				332.69		0.9020311

				332.71		0.9020311

				332.73		0.9020311

				332.75		0.9020311

				332.77		0.9020311

				332.8		0.8960573

				332.82		0.9020311

				332.84		0.8960573

				332.86		0.8960573

				332.88		0.8960573

				332.9		0.8960573

				332.92		0.8960573

				332.94		0.8960573

				332.96		0.8960573

				332.99		0.8960573

				333.01		0.9020311

				333.03		0.9020311

				333.05		0.9020311

				333.07		0.8960573

				333.09		0.8900836

				333.11		0.8960573

				333.13		0.8960573

				333.15		0.8960573

				333.18		0.8960573

				333.2		0.8960573

				333.22		0.8960573

				333.24		0.8900836

				333.26		0.8960573

				333.28		0.8960573

				333.3		0.8900836

				333.32		0.8900836

				333.34		0.8900836

				333.37		0.8900836

				333.39		0.8900836

				333.41		0.8900836

				333.43		0.8900836

				333.45		0.8960573

				333.47		0.8900836

				333.49		0.8960573

				333.51		0.8960573

				333.53		0.8960573

				333.56		0.8960573

				333.58		0.8960573

				333.6		0.8960573

				333.62		0.8960573

				333.64		0.8960573

				333.66		0.8960573

				333.68		0.8960573

				333.7		0.8960573

				333.72		0.8960573

				333.75		0.8960573

				333.77		0.8960573

				333.79		0.8960573

				333.81		0.8960573

				333.83		0.8960573

				333.85		0.8960573

				333.87		0.8960573

				333.89		0.8960573

				333.91		0.8960573

				333.94		0.8960573

				333.96		0.8960573

				333.98		0.8960573

				334		0.8960573

				334.02		0.8960573

				334.04		0.9020311

				334.06		0.8960573

				334.08		0.8960573

				334.1		0.9020311

				334.13		0.8960573

				334.15		0.8960573

				334.17		0.8960573

				334.19		0.8960573

				334.21		0.8960573

				334.23		0.8960573

				334.25		0.8960573

				334.27		0.9020311

				334.29		0.9020311

				334.32		0.9020311

				334.34		0.9020311

				334.36		0.8960573

				334.38		0.9020311

				334.4		0.9020311

				334.42		0.9020311

				334.44		0.8960573

				334.46		0.9020311

				334.48		0.8960573

				334.51		0.8960573

				334.53		0.8960573

				334.55		0.8960573

				334.57		0.8960573

				334.59		0.8960573

				334.61		0.8960573

				334.63		0.8960573

				334.65		0.8960573

				334.67		0.8960573

				334.7		0.8960573

				334.72		0.8960573

				334.74		0.8960573

				334.76		0.8960573

				334.78		0.8960573

				334.8		0.8960573

				334.82		0.8960573

				334.84		0.8960573

				334.86		0.9020311

				334.89		0.9020311

				334.91		0.8960573

				334.93		0.9020311

				334.95		0.8960573

				334.97		0.8960573

				334.99		0.8960573

				335.01		0.8960573

				335.03		0.8960573

				335.05		0.8960573

				335.08		0.8960573

				335.1		0.8900836

				335.12		0.8900836

				335.14		0.8900836

				335.16		0.8900836

				335.18		0.8900836

				335.2		0.8900836

				335.22		0.8900836

				335.24		0.8900836

				335.27		0.8900836

				335.29		0.8900836

				335.31		0.8900836

				335.33		0.8900836

				335.35		0.8900836

				335.37		0.8900836

				335.39		0.8900836

				335.41		0.8900836

				335.43		0.8900836

				335.46		0.8900836

				335.48		0.8900836

				335.5		0.8900836

				335.52		0.8900836

				335.54		0.8900836

				335.56		0.8900836

				335.58		0.8900836

				335.6		0.8900836

				335.62		0.8900836

				335.65		0.8900836

				335.67		0.8900836

				335.69		0.8900836

				335.71		0.8900836

				335.73		0.8900836

				335.75		0.8900836

				335.77		0.8900836

				335.79		0.8900836

				335.81		0.8900836

				335.84		0.8900836

				335.86		0.8900836

				335.88		0.8900836

				335.9		0.8900836

				335.92		0.8900836

				335.94		0.8900836

				335.96		0.8900836

				335.98		0.8900836

				336		0.8900836

				336.03		0.8900836

				336.05		0.8841099

				336.07		0.8841099

				336.09		0.8841099

				336.11		0.8841099

				336.13		0.8841099

				336.15		0.8841099

				336.17		0.8841099

				336.19		0.8841099

				336.22		0.8841099

				336.24		0.8841099

				336.26		0.8841099

				336.28		0.8841099

				336.3		0.8841099

				336.32		0.8841099

				336.34		0.8841099

				336.36		0.8841099

				336.38		0.8841099

				336.41		0.8841099

				336.43		0.8841099

				336.45		0.8841099

				336.47		0.8841099

				336.49		0.8841099

				336.51		0.8841099

				336.53		0.8841099

				336.55		0.8841099

				336.57		0.8841099

				336.6		0.8841099

				336.62		0.8841099

				336.64		0.8841099

				336.66		0.8841099

				336.68		0.8841099

				336.7		0.8841099

				336.72		0.8781362

				336.74		0.8781362

				336.76		0.8781362

				336.79		0.8781362

				336.81		0.8781362

				336.83		0.8781362

				336.85		0.8781362

				336.87		0.8781362

				336.89		0.8781362

				336.91		0.8781362

				336.93		0.8781362

				336.95		0.8781362

				336.98		0.8781362

				337		0.8781362

				337.02		0.8781362

				337.04		0.8781362

				337.06		0.8781362

				337.08		0.8781362

				337.1		0.8781362

				337.12		0.8841099

				337.14		0.8841099

				337.17		0.8841099

				337.19		0.8841099

				337.21		0.8841099

				337.23		0.8841099

				337.25		0.8841099

				337.27		0.8841099

				337.29		0.8841099

				337.31		0.8841099

				337.33		0.8781362

				337.36		0.8781362

				337.38		0.8841099

				337.4		0.8841099

				337.42		0.8841099

				337.44		0.8781362

				337.46		0.8781362

				337.48		0.8781362

				337.5		0.8781362

				337.52		0.8781362

				337.55		0.8781362

				337.57		0.8781362

				337.59		0.8841099

				337.61		0.8781362

				337.63		0.8841099

				337.65		0.8781362

				337.67		0.8781362

				337.69		0.8781362

				337.71		0.8781362

				337.74		0.8721625

				337.76		0.8721625

				337.78		0.8721625

				337.8		0.8661888

				337.82		0.8661888

				337.84		0.8661888

				337.86		0.8661888

				337.88		0.8661888

				337.9		0.8661888

				337.92		0.8661888

				337.95		0.8661888

				337.97		0.8661888

				337.99		0.8661888

				338.01		0.8661888

				338.03		0.8661888

				338.05		0.8602151

				338.07		0.8602151

				338.09		0.8602151

				338.11		0.8602151

				338.14		0.8602151

				338.16		0.8602151

				338.18		0.8602151

				338.2		0.8602151

				338.22		0.8602151

				338.24		0.8602151

				338.26		0.8542413

				338.28		0.8542413

				338.31		0.8542413

				338.33		0.8542413

				338.35		0.8542413

				338.37		0.8542413

				338.39		0.8542413

				338.41		0.8542413

				338.43		0.8542413

				338.45		0.8542413

				338.47		0.8542413

				338.5		0.8542413

				338.52		0.8542413

				338.54		0.8542413

				338.56		0.8542413

				338.58		0.8542413

				338.6		0.8542413

				338.62		0.8542413

				338.64		0.8542413

				338.66		0.8542413

				338.69		0.8542413

				338.71		0.8542413

				338.73		0.8542413

				338.75		0.8542413

				338.77		0.8542413

				338.79		0.8542413

				338.81		0.8542413

				338.83		0.8542413

				338.85		0.8542413

				338.88		0.8542413

				338.9		0.8542413

				338.92		0.8542413

				338.94		0.8542413

				338.96		0.8542413

				338.98		0.8542413

				339		0.8542413

				339.02		0.8542413

				339.04		0.8542413

				339.06		0.8542413

				339.09		0.8542413

				339.11		0.8542413

				339.13		0.8542413

				339.15		0.8542413

				339.17		0.8542413

				339.19		0.8542413

				339.21		0.8482676

				339.23		0.8482676

				339.25		0.8482676

				339.28		0.8482676

				339.3		0.8482676

				339.32		0.8482676

				339.34		0.8482676

				339.36		0.8482676

				339.38		0.8482676

				339.4		0.8482676

				339.42		0.8482676

				339.44		0.8482676

				339.47		0.8482676

				339.49		0.8482676

				339.51		0.8482676

				339.53		0.8482676

				339.55		0.8482676

				339.57		0.8482676

				339.59		0.8482676

				339.61		0.8482676

				339.64		0.8422939

				339.66		0.8422939

				339.68		0.8422939

				339.7		0.8422939

				339.72		0.8422939

				339.74		0.8422939

				339.76		0.8422939

				339.78		0.8482676

				339.8		0.8482676

				339.83		0.8482676

				339.85		0.8482676

				339.87		0.8482676

				339.89		0.8482676

				339.91		0.8482676

				339.93		0.8482676

				339.95		0.8482676

				339.97		0.8482676

				339.99		0.8482676

				340.02		0.8482676

				340.04		0.8482676

				340.06		0.8482676

				340.08		0.8482676

				340.1		0.8482676

				340.12		0.8482676

				340.14		0.8482676

				340.16		0.8482676

				340.19		0.8482676

				340.21		0.8482676

				340.23		0.8482676

				340.25		0.8482676

				340.27		0.8482676

				340.29		0.8482676

				340.31		0.8482676

				340.33		0.8482676

				340.35		0.8482676

				340.38		0.8482676

				340.4		0.8482676

				340.42		0.8482676

				340.44		0.8482676

				340.46		0.8482676

				340.48		0.8482676

				340.5		0.8422939

				340.52		0.8422939

				340.54		0.8422939

				340.57		0.8422939

				340.59		0.8422939

				340.61		0.8422939

				340.63		0.8363202

				340.65		0.8363202

				340.67		0.8363202

				340.69		0.8363202

				340.71		0.8363202

				340.73		0.8363202

				340.76		0.8363202

				340.78		0.8363202

				340.8		0.8363202

				340.82		0.8363202

				340.84		0.8363202

				340.86		0.8363202

				340.88		0.8363202

				340.9		0.8363202

				340.92		0.8363202

				340.95		0.8363202

				340.97		0.8363202

				340.99		0.8363202

				341.01		0.8363202

				341.03		0.8363202

				341.05		0.8363202

				341.07		0.8363202

				341.09		0.8363202

				341.11		0.8363202

				341.14		0.8363202

				341.16		0.8363202

				341.18		0.8363202

				341.2		0.8363202

				341.22		0.8303465

				341.24		0.8303465

				341.26		0.8303465

				341.28		0.8303465

				341.31		0.8303465

				341.33		0.8303465

				341.35		0.8363202

				341.37		0.8363202

				341.39		0.8303465

				341.41		0.8363202

				341.43		0.8363202

				341.45		0.8363202

				341.47		0.8363202

				341.5		0.8363202

				341.52		0.8303465

				341.54		0.8303465

				341.56		0.8303465

				341.58		0.8303465

				341.6		0.8303465

				341.62		0.8303465

				341.64		0.8303465

				341.66		0.8303465

				341.69		0.8303465

				341.71		0.8303465

				341.73		0.8303465

				341.75		0.8303465

				341.77		0.8303465

				341.79		0.8303465

				341.81		0.8303465

				341.83		0.8303465

				341.85		0.8303465

				341.88		0.8303465

				341.9		0.8303465

				341.92		0.8303465

				341.94		0.8243728

				341.96		0.8243728

				341.98		0.8243728

				342		0.8243728

				342.02		0.8243728

				342.04		0.8243728

				342.07		0.8243728

				342.09		0.8243728

				342.11		0.8243728

				342.13		0.8243728

				342.15		0.8243728

				342.17		0.8243728

				342.19		0.8243728

				342.21		0.8243728

				342.24		0.8243728

				342.26		0.8243728

				342.28		0.8243728

				342.3		0.8243728

				342.32		0.8243728

				342.34		0.8243728

				342.36		0.8243728

				342.38		0.8243728

				342.4		0.8243728

				342.43		0.8243728

				342.45		0.8243728

				342.47		0.8243728

				342.49		0.8243728

				342.51		0.8243728

				342.53		0.8243728

				342.55		0.8243728

				342.57		0.8243728

				342.59		0.8243728

				342.62		0.8243728

				342.64		0.8243728

				342.66		0.8243728

				342.68		0.8243728

				342.7		0.8243728

				342.72		0.8243728

				342.74		0.8243728

				342.76		0.8243728

				342.78		0.8243728

				342.81		0.8243728

				342.83		0.8243728

				342.85		0.8243728

				342.87		0.8243728

				342.89		0.8243728

				342.91		0.8243728

				342.93		0.8243728

				342.95		0.8243728

				342.97		0.8243728

				343		0.8243728

				343.02		0.8243728

				343.04		0.8243728

				343.06		0.8243728

				343.08		0.8243728

				343.1		0.8243728

				343.12		0.8243728

				343.14		0.8243728

				343.16		0.8243728

				343.19		0.8243728

				343.21		0.8243728

				343.23		0.8243728

				343.25		0.8243728

				343.27		0.8243728

				343.29		0.8243728

				343.31		0.8243728

				343.33		0.8243728

				343.35		0.8243728

				343.38		0.8243728

				343.4		0.8243728

				343.42		0.8243728

				343.44		0.8243728

				343.46		0.8243728

				343.48		0.8243728

				343.5		0.8243728

				343.52		0.8243728

				343.55		0.8243728

				343.57		0.8243728

				343.59		0.8243728

				343.61		0.8243728

				343.63		0.8243728

				343.65		0.8243728

				343.67		0.8243728

				343.69		0.8243728

				343.71		0.8243728

				343.74		0.8243728

				343.76		0.8243728

				343.78		0.8243728

				343.8		0.8243728

				343.82		0.8243728

				343.84		0.8243728

				343.86		0.8243728

				343.88		0.8243728

				343.9		0.8243728

				343.93		0.8243728

				343.95		0.8243728

				343.97		0.8243728

				343.99		0.8243728

				344.01		0.8243728

				344.03		0.8243728

				344.05		0.8243728

				344.07		0.8243728

				344.09		0.8243728

				344.12		0.8243728

				344.14		0.8243728

				344.16		0.8243728

				344.18		0.8243728

				344.2		0.8243728

				344.22		0.8243728

				344.24		0.8243728

				344.26		0.8243728

				344.29		0.8243728

				344.31		0.8243728

				344.33		0.8243728

				344.35		0.8243728

				344.37		0.8243728

				344.39		0.8243728

				344.41		0.8243728

				344.43		0.8243728

				344.45		0.8243728

				344.48		0.8243728

				344.5		0.8243728

				344.52		0.8243728

				344.54		0.8243728

				344.56		0.8243728

				344.58		0.8243728

				344.6		0.8243728

				344.62		0.8243728

				344.64		0.8243728

				344.67		0.818399

				344.69		0.818399

				344.71		0.818399

				344.73		0.818399

				344.75		0.818399

				344.77		0.8243728

				344.79		0.8243728

				344.81		0.8243728

				344.83		0.8243728

				344.86		0.8243728

				344.88		0.8243728

				344.9		0.8243728

				344.92		0.8243728

				344.94		0.8243728

				344.96		0.8243728

				344.98		0.8243728

				345		0.8243728

				345.02		0.818399

				345.05		0.818399

				345.07		0.8243728

				345.09		0.818399

				345.11		0.818399

				345.13		0.818399

				345.15		0.818399

				345.17		0.818399

				345.19		0.818399

				345.22		0.818399

				345.24		0.818399

				345.26		0.818399

				345.28		0.818399

				345.3		0.818399

				345.32		0.818399

				345.34		0.818399

				345.36		0.818399

				345.38		0.818399

				345.41		0.818399

				345.43		0.818399

				345.45		0.818399

				345.47		0.818399

				345.49		0.818399

				345.51		0.8124253

				345.53		0.8124253

				345.55		0.8124253

				345.57		0.8124253

				345.6		0.8124253

				345.62		0.8124253

				345.64		0.8124253

				345.66		0.8124253

				345.68		0.8124253

				345.7		0.8124253

				345.72		0.8124253

				345.74		0.8124253

				345.77		0.8124253

				345.79		0.8124253

				345.81		0.8124253

				345.83		0.8124253

				345.85		0.8124253

				345.87		0.8124253

				345.89		0.8124253

				345.91		0.8124253

				345.93		0.8064516

				345.96		0.8124253

				345.98		0.8064516

				346		0.8064516

				346.02		0.8064516

				346.04		0.8064516

				346.06		0.8064516

				346.08		0.8064516

				346.1		0.8064516

				346.12		0.8064516

				346.15		0.8064516

				346.17		0.8064516

				346.19		0.8124253

				346.21		0.8124253

				346.23		0.8124253

				346.25		0.8064516

				346.27		0.8124253

				346.29		0.8064516

				346.32		0.8064516

				346.34		0.8064516

				346.36		0.8064516

				346.38		0.8064516

				346.4		0.8064516

				346.42		0.8064516

				346.44		0.8064516

				346.46		0.8064516

				346.48		0.8064516

				346.51		0.8064516

				346.53		0.8064516

				346.55		0.8064516

				346.57		0.8064516

				346.59		0.8064516

				346.61		0.8124253

				346.63		0.8064516

				346.65		0.8064516

				346.67		0.8064516

				346.7		0.8064516

				346.72		0.8064516

				346.74		0.8064516

				346.76		0.8064516

				346.78		0.8064516

				346.8		0.8064516

				346.82		0.8064516

				346.84		0.8064516

				346.86		0.8064516

				346.89		0.8064516

				346.91		0.8064516

				346.93		0.8064516

				346.95		0.8064516

				346.97		0.8064516

				346.99		0.8064516

				347.01		0.8064516

				347.03		0.8064516

				347.06		0.8064516

				347.08		0.8064516

				347.1		0.8064516

				347.12		0.8064516

				347.14		0.8064516

				347.16		0.8064516

				347.18		0.8064516

				347.2		0.8064516

				347.22		0.8064516

				347.25		0.8064516

				347.27		0.8004779

				347.29		0.8004779

				347.31		0.8004779

				347.33		0.8064516

				347.35		0.8004779

				347.37		0.8064516

				347.39		0.8064516

				347.42		0.8064516

				347.44		0.8064516

				347.46		0.8064516

				347.48		0.8064516

				347.5		0.8064516

				347.52		0.8004779

				347.54		0.8064516

				347.56		0.8064516

				347.58		0.8064516

				347.61		0.8064516

				347.63		0.8064516

				347.65		0.8004779

				347.67		0.8064516

				347.69		0.8064516

				347.71		0.8064516

				347.73		0.8064516

				347.75		0.8064516

				347.77		0.8064516

				347.8		0.8064516

				347.82		0.8004779

				347.84		0.8004779

				347.86		0.8064516

				347.88		0.8004779

				347.9		0.8004779

				347.92		0.8004779

				347.94		0.8004779

				347.97		0.8004779

				347.99		0.8004779

				348.01		0.8004779

				348.03		0.8004779

				348.05		0.8004779

				348.07		0.8064516

				348.09		0.8064516

				348.11		0.8064516

				348.13		0.8064516

				348.16		0.8064516

				348.18		0.8064516

				348.2		0.8064516

				348.22		0.8064516

				348.24		0.8064516

				348.26		0.8064516

				348.28		0.8004779

				348.3		0.8004779

				348.32		0.8064516

				348.35		0.8064516

				348.37		0.8004779

				348.39		0.8064516

				348.41		0.8004779

				348.43		0.8004779

				348.45		0.8004779

				348.47		0.8004779

				348.49		0.8064516

				348.52		0.8004779

				348.54		0.8004779

				348.56		0.8004779

				348.58		0.8004779

				348.6		0.8004779

				348.62		0.8004779

				348.64		0.8004779

				348.66		0.8004779

				348.68		0.8004779

				348.71		0.8004779

				348.73		0.8004779

				348.75		0.8064516

				348.77		0.8004779

				348.79		0.8004779

				348.81		0.8064516

				348.83		0.8064516

				348.85		0.8004779

				348.88		0.8064516

				348.9		0.8064516

				348.92		0.8064516

				348.94		0.8064516

				348.96		0.8064516

				348.98		0.8064516

				349		0.8064516

				349.02		0.8064516

				349.04		0.8064516

				349.07		0.8064516

				349.09		0.8064516

				349.11		0.8064516

				349.13		0.8064516

				349.15		0.8064516

				349.17		0.8064516

				349.19		0.8064516

				349.21		0.8064516

				349.24		0.8064516

				349.26		0.8064516

				349.28		0.8064516

				349.3		0.8064516

				349.32		0.8064516

				349.34		0.8064516

				349.36		0.8064516

				349.39		0.8064516

				349.41		0.8064516

				349.43		0.8064516

				349.45		0.8064516

				349.47		0.8064516

				349.49		0.8064516

				349.51		0.8064516

				349.53		0.8064516

				349.56		0.8064516

				349.58		0.8064516

				349.6		0.8064516

				349.62		0.8064516

				349.64		0.8064516

				349.66		0.8064516

				349.68		0.8064516

				349.71		0.8064516

				349.73		0.8064516

				349.75		0.8064516

				349.77		0.8064516

				349.79		0.8064516

				349.81		0.8064516

				349.83		0.8064516

				349.86		0.8064516

				349.88		0.8064516

				349.9		0.8064516

				349.92		0.8064516

				349.94		0.8064516

				349.96		0.8064516

				349.98		0.8064516

				350.01		0.8064516

				350.03		0.8064516

				350.05		0.8124253

				350.07		0.8064516

				350.09		0.8124253

				350.11		0.8124253

				350.13		0.8124253

				350.16		0.8124253

				350.18		0.8064516

				350.2		0.8124253

				350.22		0.8124253

				350.24		0.8124253

				350.26		0.8064516

				350.28		0.8124253

				350.3		0.8064516

				350.33		0.8124253

				350.35		0.8064516

				350.37		0.8124253

				350.39		0.8124253

				350.41		0.8124253

				350.43		0.8064516

				350.45		0.8124253

				350.47		0.8124253

				350.5		0.8064516

				350.52		0.8124253

				350.54		0.8124253

				350.56		0.8124253

				350.58		0.8124253

				350.6		0.8064516

				350.62		0.8124253

				350.64		0.8124253

				350.66		0.8124253

				350.69		0.8124253

				350.71		0.8124253

				350.73		0.8124253

				350.75		0.8124253

				350.77		0.8124253

				350.79		0.8124253

				350.81		0.8124253

				350.83		0.8124253

				350.86		0.8124253

				350.88		0.8124253

				350.9		0.8124253

				350.92		0.8124253

				350.94		0.8124253

				350.96		0.8124253

				350.98		0.8124253

				351		0.8124253

				351.02		0.8124253

				351.05		0.8124253

				351.07		0.8124253

				351.09		0.8124253

				351.11		0.8124253

				351.13		0.8124253

				351.15		0.8124253

				351.17		0.8124253

				351.19		0.8124253

				351.22		0.8124253

				351.24		0.8124253

				351.26		0.8124253

				351.28		0.8124253

				351.3		0.8124253

				351.32		0.8124253

				351.34		0.8124253

				351.36		0.8064516

				351.39		0.8124253

				351.41		0.8124253

				351.43		0.8124253

				351.45		0.8124253

				351.47		0.8124253

				351.49		0.8064516

				351.51		0.8064516

				351.53		0.8064516

				351.56		0.8124253

				351.58		0.8124253

				351.6		0.8064516

				351.62		0.8064516

				351.64		0.8064516

				351.66		0.8064516

				351.68		0.8064516

				351.7		0.8124253

				351.73		0.8124253

				351.75		0.8124253

				351.77		0.8064516

				351.79		0.8064516

				351.81		0.8124253

				351.83		0.8064516

				351.85		0.8064516

				351.87		0.8064516

				351.9		0.8064516

				351.92		0.8064516

				351.94		0.8064516

				351.96		0.8064516

				351.98		0.8064516

				352		0.8064516

				352.02		0.8064516

				352.04		0.8064516

				352.07		0.8064516

				352.09		0.8064516

				352.11		0.8064516

				352.13		0.8064516

				352.15		0.8064516

				352.17		0.8004779

				352.19		0.8004779

				352.21		0.8004779

				352.24		0.8004779

				352.26		0.8004779

				352.28		0.8004779

				352.3		0.8004779

				352.32		0.8004779

				352.34		0.8004779

				352.36		0.8004779

				352.38		0.8004779

				352.41		0.8004779

				352.43		0.8064516

				352.45		0.8064516

				352.47		0.8004779

				352.49		0.8004779

				352.51		0.8004779

				352.53		0.8004779

				352.55		0.8004779

				352.58		0.8004779

				352.6		0.8004779

				352.62		0.8004779

				352.64		0.8004779

				352.66		0.8004779

				352.68		0.8004779

				352.7		0.8004779

				352.72		0.8004779

				352.75		0.8004779

				352.77		0.8004779

				352.79		0.8004779

				352.81		0.8004779

				352.83		0.8004779

				352.85		0.8004779

				352.87		0.8004779

				352.89		0.8004779

				352.92		0.8004779

				352.94		0.8004779

				352.96		0.8004779

				352.98		0.8004779

				353		0.8004779

				353.02		0.8004779

				353.04		0.8004779

				353.06		0.8004779

				353.09		0.8004779

				353.11		0.8004779

				353.13		0.8004779

				353.15		0.8004779

				353.17		0.8004779

				353.19		0.8004779

				353.21		0.8004779

				353.23		0.8004779

				353.26		0.8004779

				353.28		0.8004779

				353.3		0.7945042

				353.32		0.7945042

				353.34		0.7945042

				353.36		0.7945042

				353.38		0.7945042

				353.4		0.7945042

				353.43		0.7945042

				353.45		0.7945042

				353.47		0.7945042

				353.49		0.7945042

				353.51		0.7945042

				353.53		0.7945042

				353.55		0.7945042

				353.58		0.7945042

				353.6		0.7945042

				353.62		0.7945042

				353.64		0.7945042

				353.66		0.7945042

				353.68		0.7945042

				353.7		0.7945042

				353.72		0.7885305

				353.75		0.7885305

				353.77		0.7885305

				353.79		0.7885305

				353.81		0.7885305

				353.83		0.7885305

				353.85		0.7885305

				353.87		0.7885305

				353.89		0.7885305

				353.92		0.7885305

				353.94		0.7885305

				353.96		0.7885305

				353.98		0.7885305

				354		0.7885305

				354.02		0.7885305

				354.04		0.7885305

				354.06		0.7885305

				354.09		0.7885305

				354.11		0.7885305

				354.13		0.7885305

				354.15		0.7885305

				354.17		0.7885305

				354.19		0.7825568

				354.21		0.7825568

				354.23		0.7825568

				354.26		0.7825568

				354.28		0.7825568

				354.3		0.7825568

				354.32		0.7825568

				354.34		0.7825568

				354.36		0.7825568

				354.38		0.7825568

				354.4		0.7825568

				354.43		0.7825568

				354.45		0.7825568

				354.47		0.7825568

				354.49		0.7825568

				354.51		0.7825568

				354.53		0.776583

				354.55		0.776583

				354.57		0.7825568

				354.6		0.7825568

				354.62		0.7825568

				354.64		0.7825568

				354.66		0.7825568

				354.68		0.7825568

				354.7		0.7825568

				354.72		0.7825568

				354.74		0.7825568

				354.77		0.776583

				354.79		0.776583

				354.81		0.776583

				354.83		0.776583

				354.85		0.776583

				354.87		0.776583

				354.89		0.776583

				354.91		0.776583

				354.94		0.776583

				354.96		0.776583

				354.98		0.776583

				355		0.776583

				355.02		0.776583

				355.04		0.776583

				355.06		0.776583

				355.08		0.776583

				355.11		0.776583

				355.13		0.776583

				355.15		0.776583

				355.17		0.776583

				355.19		0.776583

				355.21		0.776583

				355.23		0.776583

				355.25		0.776583

				355.28		0.776583

				355.3		0.776583

				355.32		0.776583

				355.34		0.776583

				355.36		0.776583

				355.38		0.776583

				355.4		0.776583

				355.42		0.776583

				355.45		0.776583

				355.47		0.776583

				355.49		0.776583

				355.51		0.776583

				355.53		0.776583

				355.55		0.776583

				355.57		0.776583

				355.59		0.776583

				355.62		0.776583

				355.64		0.776583

				355.66		0.776583

				355.68		0.776583

				355.7		0.776583

				355.72		0.776583

				355.74		0.776583

				355.77		0.776583

				355.79		0.776583

				355.81		0.776583

				355.83		0.776583

				355.85		0.776583

				355.87		0.7825568

				355.89		0.776583

				355.91		0.7825568

				355.94		0.7825568

				355.96		0.7825568

				355.98		0.7825568

				356		0.7825568

				356.02		0.7825568

				356.04		0.7825568

				356.06		0.7825568

				356.08		0.7825568

				356.11		0.7825568

				356.13		0.7825568

				356.15		0.7825568

				356.17		0.7825568

				356.19		0.7825568

				356.21		0.7825568

				356.23		0.7825568

				356.25		0.7825568

				356.28		0.7825568

				356.3		0.7825568

				356.32		0.7825568

				356.34		0.7825568

				356.36		0.7825568

				356.38		0.7825568

				356.4		0.7825568

				356.42		0.7825568

				356.45		0.7825568

				356.47		0.7825568

				356.49		0.7825568

				356.51		0.7825568

				356.53		0.7825568

				356.55		0.7825568

				356.57		0.7825568

				356.6		0.7885305

				356.62		0.7885305

				356.64		0.7885305

				356.66		0.7885305

				356.68		0.7885305

				356.7		0.7885305

				356.72		0.7885305

				356.74		0.7885305

				356.77		0.7885305

				356.79		0.7885305

				356.81		0.7885305

				356.83		0.7885305

				356.85		0.7825568

				356.87		0.7885305

				356.89		0.7885305

				356.91		0.7885305

				356.94		0.7825568

				356.96		0.7825568

				356.98		0.7885305

				357		0.7885305

				357.02		0.7885305

				357.04		0.7825568

				357.06		0.7885305

				357.08		0.7825568

				357.11		0.7885305

				357.13		0.7825568

				357.15		0.7885305

				357.17		0.7825568

				357.19		0.7825568

				357.21		0.7825568

				357.23		0.7825568

				357.25		0.7825568

				357.28		0.7825568

				357.3		0.7825568

				357.32		0.7825568

				357.34		0.7825568

				357.36		0.7825568

				357.38		0.7825568

				357.4		0.7825568

				357.42		0.7825568

				357.45		0.7825568

				357.47		0.7825568

				357.49		0.7825568

				357.51		0.7825568

				357.53		0.7825568

				357.55		0.7825568

				357.57		0.7825568

				357.59		0.7825568

				357.62		0.7825568

				357.64		0.7825568

				357.66		0.7825568

				357.68		0.7825568

				357.7		0.7825568

				357.72		0.7825568

				357.74		0.776583

				357.76		0.776583

				357.79		0.776583

				357.81		0.776583

				357.83		0.776583

				357.85		0.776583

				357.87		0.776583

				357.89		0.776583

				357.91		0.776583

				357.93		0.776583

				357.96		0.7706093

				357.98		0.7706093

				358		0.7706093

				358.02		0.7706093

				358.04		0.7706093

				358.06		0.7706093

				358.08		0.7706093

				358.1		0.7706093

				358.13		0.7706093

				358.15		0.7706093

				358.17		0.7706093

				358.19		0.7706093

				358.21		0.7706093

				358.23		0.7706093

				358.25		0.7706093

				358.27		0.7646356

				358.3		0.7646356

				358.32		0.7646356

				358.34		0.7646356

				358.36		0.7646356

				358.38		0.7646356

				358.4		0.7646356

				358.42		0.7646356

				358.44		0.7646356

				358.47		0.7646356

				358.49		0.7586619

				358.51		0.7586619

				358.53		0.7646356

				358.55		0.7586619

				358.57		0.7586619

				358.59		0.7586619

				358.61		0.7586619

				358.64		0.7586619

				358.66		0.7586619

				358.68		0.7586619

				358.7		0.7526882

				358.72		0.7526882

				358.74		0.7526882

				358.76		0.7526882

				358.78		0.7526882

				358.81		0.7526882

				358.83		0.7526882

				358.85		0.7526882

				358.87		0.7526882

				358.89		0.7526882

				358.91		0.7526882

				358.93		0.7526882

				358.95		0.7526882

				358.98		0.7526882

				359		0.7526882

				359.02		0.7526882

				359.04		0.7526882

				359.06		0.7526882

				359.08		0.7526882

				359.1		0.7467145

				359.12		0.7467145

				359.15		0.7467145

				359.17		0.7467145

				359.19		0.7467145

				359.21		0.7467145

				359.23		0.7467145

				359.25		0.7467145

				359.27		0.7407407

				359.29		0.7407407

				359.32		0.7407407

				359.34		0.7407407

				359.36		0.7407407

				359.38		0.7407407

				359.4		0.7407407

				359.42		0.7407407

				359.44		0.7407407

				359.46		0.7407407

				359.49		0.7407407

				359.51		0.7407407

				359.53		0.7407407

				359.55		0.7407407

				359.57		0.7407407

				359.59		0.7407407

				359.61		0.7407407

				359.63		0.7407407

				359.66		0.7407407

				359.68		0.7407407

				359.7		0.7407407

				359.72		0.734767

				359.74		0.734767

				359.76		0.734767

				359.78		0.734767

				359.81		0.734767

				359.83		0.734767

				359.85		0.734767

				359.87		0.734767

				359.89		0.734767

				359.91		0.734767

				359.93		0.734767

				359.95		0.734767

				359.98		0.734767

				360		0.734767

				360.02		0.734767

				360.04		0.7407407

				360.06		0.7407407

				360.08		0.7407407

				360.1		0.7407407

				360.12		0.7407407

				360.15		0.7407407

				360.17		0.7407407

				360.19		0.7407407

				360.21		0.7407407

				360.23		0.7407407

				360.25		0.7407407

				360.27		0.7407407

				360.29		0.7407407

				360.32		0.7407407

				360.34		0.7407407

				360.36		0.7407407

				360.38		0.7407407

				360.4		0.7407407

				360.42		0.7407407

				360.44		0.7407407

				360.46		0.7407407

				360.49		0.7407407

				360.51		0.7407407

				360.53		0.7407407

				360.55		0.7407407

				360.57		0.7407407

				360.59		0.7407407

				360.61		0.7407407

				360.63		0.7407407

				360.66		0.7407407

				360.68		0.7407407

				360.7		0.7407407

				360.72		0.7407407

				360.74		0.7407407

				360.76		0.7407407

				360.78		0.7407407

				360.8		0.7407407

				360.83		0.7407407

				360.85		0.7407407

				360.87		0.7407407

				360.89		0.7407407

				360.91		0.7407407

				360.93		0.7407407

				360.95		0.7407407

				360.98		0.7407407

				361		0.7407407

				361.02		0.7407407

				361.04		0.7407407

				361.06		0.7407407

				361.08		0.7407407

				361.1		0.7407407

				361.12		0.7407407

				361.15		0.7407407

				361.17		0.7407407

				361.19		0.7407407

				361.21		0.7407407

				361.23		0.7407407

				361.25		0.7407407

				361.27		0.7407407

				361.29		0.7407407

				361.32		0.7407407

				361.34		0.7407407

				361.36		0.7407407

				361.38		0.7407407

				361.4		0.7407407

				361.42		0.7407407

				361.44		0.7407407

				361.46		0.7407407

				361.49		0.7407407

				361.51		0.7407407

				361.53		0.7467145

				361.55		0.7407407

				361.57		0.7407407

				361.59		0.7407407

				361.61		0.7407407

				361.63		0.7407407

				361.66		0.7407407

				361.68		0.7407407

				361.7		0.7407407

				361.72		0.7407407

				361.74		0.7467145

				361.76		0.7467145

				361.78		0.7467145

				361.8		0.7407407

				361.83		0.7407407

				361.85		0.7467145

				361.87		0.7467145

				361.89		0.7467145

				361.91		0.7467145

				361.93		0.7407407

				361.95		0.7407407

				361.97		0.7407407

				362		0.7407407

				362.02		0.7407407

				362.04		0.7407407

				362.06		0.7407407

				362.08		0.7407407

				362.1		0.7407407

				362.12		0.7407407

				362.14		0.7407407

				362.17		0.7407407

				362.19		0.7407407

				362.21		0.7407407

				362.23		0.7407407

				362.25		0.7407407

				362.27		0.7407407

				362.29		0.7407407

				362.31		0.7407407

				362.34		0.7407407

				362.36		0.7407407

				362.38		0.7407407

				362.4		0.7407407

				362.42		0.7407407

				362.44		0.7407407

				362.46		0.7407407

				362.48		0.7407407

				362.51		0.7407407

				362.53		0.7407407

				362.55		0.7407407

				362.57		0.7407407

				362.59		0.7407407

				362.61		0.7407407

				362.63		0.7407407

				362.65		0.7407407

				362.68		0.7407407

				362.7		0.7407407

				362.72		0.7407407

				362.74		0.7407407

				362.76		0.7407407

				362.78		0.7407407

				362.8		0.7407407

				362.82		0.7407407

				362.85		0.7407407

				362.87		0.7407407

				362.89		0.7407407

				362.91		0.7407407

				362.93		0.7407407

				362.95		0.7407407

				362.97		0.7407407

				362.99		0.7407407

				363.02		0.7407407

				363.04		0.7407407

				363.06		0.7407407

				363.08		0.7407407

				363.1		0.7407407

				363.12		0.7407407

				363.14		0.7407407

				363.16		0.7407407

				363.19		0.7407407

				363.21		0.7407407

				363.23		0.7407407

				363.25		0.7407407

				363.27		0.7407407

				363.29		0.7407407

				363.31		0.7407407

				363.33		0.7407407

				363.35		0.7407407

				363.38		0.7407407

				363.4		0.7407407

				363.42		0.7407407

				363.44		0.7407407

				363.46		0.7407407

				363.48		0.7407407

				363.5		0.7407407

				363.52		0.7407407

				363.55		0.7407407

				363.57		0.7407407

				363.59		0.7407407

				363.61		0.7407407

				363.63		0.7407407

				363.65		0.7407407

				363.67		0.7407407

				363.69		0.7407407

				363.72		0.7407407

				363.74		0.7407407

				363.76		0.7407407

				363.78		0.7407407

				363.8		0.7407407

				363.82		0.7407407

				363.84		0.7407407

				363.86		0.7407407

				363.89		0.7407407

				363.91		0.7407407

				363.93		0.7407407

				363.95		0.734767

				363.97		0.7407407

				363.99		0.734767

				364.01		0.734767

				364.03		0.734767

				364.05		0.734767

				364.08		0.734767

				364.1		0.734767

				364.12		0.7407407

				364.14		0.734767

				364.16		0.734767

				364.18		0.734767

				364.2		0.734767

				364.22		0.734767

				364.25		0.734767

				364.27		0.734767

				364.29		0.734767

				364.31		0.734767

				364.33		0.734767

				364.35		0.734767

				364.37		0.734767

				364.39		0.734767

				364.42		0.734767

				364.44		0.734767

				364.46		0.734767

				364.48		0.734767

				364.5		0.734767

				364.52		0.734767

				364.54		0.734767

				364.56		0.734767

				364.59		0.734767

				364.61		0.734767

				364.63		0.734767

				364.65		0.734767

				364.67		0.734767

				364.69		0.734767

				364.71		0.734767

				364.73		0.734767

				364.76		0.7287933

				364.78		0.7287933

				364.8		0.7287933

				364.82		0.7287933

				364.84		0.7287933

				364.86		0.7287933

				364.88		0.7287933

				364.91		0.7287933

				364.93		0.7287933

				364.95		0.7287933

				364.97		0.7228196

				364.99		0.7228196

				365.01		0.7228196

				365.03		0.7228196

				365.05		0.7228196

				365.08		0.7168459

				365.1		0.6869773

				365.12		0.6630824

				365.14		0.6571087

				365.16		0.6571087

				365.18		0.6571087

				365.2		0.651135

				365.22		0.651135

				365.25		0.651135

				365.27		0.651135

				365.29		0.6571087

				365.31		0.6571087

				365.33		0.6630824

				365.35		0.6630824

				365.37		0.6690562

				365.39		0.6690562

				365.42		0.6690562

				365.44		0.6750299

				365.46		0.6750299

				365.48		0.6750299

				365.5		0.6810036

				365.52		0.6810036

				365.54		0.6810036

				365.56		0.6869773

				365.59		0.7168459

				365.61		0.7168459

				365.63		0.7108722

				365.65		0.7108722

				365.67		0.7108722

				365.69		0.7108722

				365.71		0.7108722

				365.73		0.7108722

				365.75		0.7108722

				365.78		0.7168459

				365.8		0.7108722

				365.82		0.7108722

				365.84		0.7108722

				365.86		0.7168459

				365.88		0.7168459

				365.9		0.7108722

				365.92		0.7168459

				365.95		0.7168459

				365.97		0.7108722

				365.99		0.7108722

				366.01		0.7108722

				366.03		0.7467145

				366.05		0.7885305

				366.07		0.7945042

				366.09		0.8064516

				366.11		0.8124253

				366.14		0.818399

				366.16		0.8243728

				366.18		0.8363202

				366.2		0.8542413

				366.22		0.8661888

				366.24		0.8781362

				366.26		0.8781362

				366.28		0.8841099

				366.31		0.8781362

				366.33		0.8661888

				366.35		0.8661888

				366.37		0.8542413

				366.39		0.8422939

				366.41		0.8363202

				366.43		0.8303465

				366.45		0.8243728

				366.48		0.818399

				366.5		0.8124253

				366.52		0.8064516

				366.54		0.8004779

				366.56		0.8004779

				366.58		0.7945042

				366.6		0.7945042

				366.62		0.7885305

				366.65		0.7885305

				366.67		0.7825568

				366.69		0.7825568

				366.71		0.7885305

				366.73		0.7885305

				366.75		0.7885305

				366.77		0.7885305

				366.8		0.7945042

				366.82		0.7945042

				366.84		0.7885305

				366.86		0.7706093

				366.88		0.734767

				366.9		0.7108722

				366.92		0.7048984

				366.95		0.7048984

				366.97		0.7108722

				366.99		0.7048984

				367.01		0.7048984

				367.03		0.7048984

				367.05		0.7048984

				367.07		0.7048984

				367.09		0.7048984

				367.12		0.7048984

				367.14		0.7048984

				367.16		0.7108722

				367.18		0.7108722

				367.2		0.7108722

				367.22		0.7108722

				367.24		0.7108722

				367.26		0.7108722

				367.29		0.7108722

				367.31		0.7108722

				367.33		0.7108722

				367.35		0.7108722

				367.37		0.7108722

				367.39		0.7108722

				367.41		0.7108722

				367.44		0.7108722

				367.46		0.7108722

				367.48		0.7108722

				367.5		0.7108722

				367.52		0.7108722

				367.54		0.7108722

				367.56		0.7108722

				367.58		0.7108722

				367.61		0.7048984

				367.63		0.7108722

				367.65		0.7108722

				367.67		0.7108722

				367.69		0.7108722

				367.71		0.7108722

				367.73		0.7108722

				367.75		0.7048984

				367.78		0.7048984

				367.8		0.7048984

				367.82		0.7048984

				367.84		0.7048984

				367.86		0.7048984

				367.88		0.7048984

				367.9		0.7048984

				367.92		0.7048984

				367.95		0.7048984

				367.97		0.7048984

				367.99		0.7048984

				368.01		0.7048984

				368.03		0.7048984

				368.05		0.7048984

				368.07		0.7048984

				368.09		0.7048984

				368.12		0.7048984

				368.14		0.7048984

				368.16		0.7048984

				368.18		0.7048984

				368.2		0.7048984

				368.22		0.7048984

				368.24		0.7048984

				368.26		0.7048984

				368.29		0.7048984

				368.31		0.7048984

				368.33		0.7048984

				368.35		0.7048984

				368.37		0.7048984

				368.39		0.7048984

				368.41		0.7048984

				368.43		0.7048984

				368.46		0.7048984

				368.48		0.7048984

				368.5		0.7048984

				368.52		0.7048984

				368.54		0.7048984

				368.56		0.7048984

				368.58		0.7048984

				368.6		0.7048984

				368.63		0.7048984

				368.65		0.7048984

				368.67		0.7048984

				368.69		0.6989247

				368.71		0.6989247

				368.73		0.6989247

				368.75		0.6989247

				368.77		0.6989247

				368.8		0.6989247

				368.82		0.6989247

				368.84		0.6989247

				368.86		0.6989247

				368.88		0.6989247

				368.9		0.6989247

				368.92		0.6989247

				368.94		0.6989247

				368.97		0.6989247

				368.99		0.6989247

				369.01		0.7048984

				369.03		0.7048984

				369.05		0.7048984

				369.07		0.7048984

				369.09		0.7048984

				369.11		0.7048984

				369.14		0.7048984

				369.16		0.7048984

				369.18		0.7048984

				369.2		0.7048984

				369.22		0.7048984

				369.24		0.7048984

				369.26		0.7048984

				369.28		0.7048984

				369.31		0.7048984

				369.33		0.7048984

				369.35		0.7048984

				369.37		0.7048984

				369.39		0.7048984

				369.41		0.7048984

				369.43		0.7048984

				369.45		0.7048984

				369.48		0.7048984

				369.5		0.7048984

				369.52		0.7048984

				369.54		0.7048984

				369.56		0.7048984

				369.58		0.7048984

				369.6		0.7048984

				369.62		0.7048984

				369.65		0.7048984

				369.67		0.7048984

				369.69		0.7048984

				369.71		0.7048984

				369.73		0.7048984

				369.75		0.7048984

				369.77		0.7048984

				369.79		0.7048984

				369.82		0.7048984

				369.84		0.7048984

				369.86		0.7048984

				369.88		0.7048984

				369.9		0.7048984

				369.92		0.7048984

				369.94		0.7048984

				369.96		0.7048984

				369.99		0.7048984

				370.01		0.7048984

				370.03		0.7048984

				370.05		0.7048984

				370.07		0.7048984

				370.09		0.7048984

				370.11		0.7048984

				370.14		0.7048984

				370.16		0.7108722

				370.18		0.7108722

				370.2		0.7108722

				370.22		0.7108722

				370.24		0.7108722

				370.26		0.7108722

				370.28		0.7108722

				370.31		0.7108722

				370.33		0.7108722

				370.35		0.7108722

				370.37		0.7108722

				370.39		0.7108722

				370.41		0.7108722

				370.43		0.7108722

				370.45		0.7108722

				370.48		0.7108722

				370.5		0.7108722

				370.52		0.7108722

				370.54		0.7108722

				370.56		0.7108722

				370.58		0.7108722

				370.6		0.7108722

				370.62		0.7108722

				370.65		0.7108722

				370.67		0.7108722

				370.69		0.7108722

				370.71		0.7048984

				370.73		0.7048984

				370.75		0.7048984

				370.77		0.7048984

				370.79		0.7048984

				370.82		0.7048984

				370.84		0.7108722

				370.86		0.7048984

				370.88		0.7108722

				370.9		0.7108722

				370.92		0.7108722

				370.94		0.7108722

				370.96		0.7108722

				370.99		0.7108722

				371.01		0.7108722

				371.03		0.7108722

				371.05		0.7108722

				371.07		0.7108722

				371.09		0.7108722

				371.11		0.7048984

				371.13		0.7048984

				371.16		0.7048984

				371.18		0.7048984

				371.2		0.7048984

				371.22		0.7048984

				371.24		0.7048984

				371.26		0.7048984

				371.28		0.7048984

				371.3		0.7048984

				371.33		0.7048984

				371.35		0.7048984

				371.37		0.7048984

				371.39		0.7048984

				371.41		0.7048984

				371.43		0.7048984

				371.45		0.7048984

				371.48		0.7048984

				371.5		0.7048984

				371.52		0.7048984

				371.54		0.7048984

				371.56		0.7048984

				371.58		0.7048984

				371.6		0.7048984

				371.62		0.7048984

				371.65		0.7048984

				371.67		0.7048984

				371.69		0.7048984

				371.71		0.7048984

				371.73		0.7048984

				371.75		0.7048984

				371.77		0.7048984

				371.79		0.7048984

				371.82		0.7048984

				371.84		0.7048984

				371.86		0.7048984

				371.88		0.7048984

				371.9		0.7048984

				371.92		0.7048984

				371.94		0.7048984

				371.96		0.7048984

				371.99		0.7048984

				372.01		0.7048984

				372.03		0.7048984

				372.05		0.7048984

				372.07		0.7048984

				372.09		0.7048984

				372.11		0.7048984

				372.13		0.7048984

				372.16		0.7048984

				372.18		0.7048984

				372.2		0.7048984

				372.22		0.7048984

				372.24		0.7048984

				372.26		0.7048984

				372.28		0.7048984

				372.31		0.7048984

				372.33		0.7048984

				372.35		0.7048984

				372.37		0.7048984

				372.39		0.7048984

				372.41		0.7048984

				372.43		0.7048984

				372.45		0.7048984

				372.48		0.7048984

				372.5		0.7048984

				372.52		0.7048984

				372.54		0.7048984

				372.56		0.7048984

				372.58		0.7048984

				372.6		0.7048984

				372.62		0.7048984

				372.65		0.7048984

				372.67		0.7048984

				372.69		0.7048984

				372.71		0.7048984

				372.73		0.7048984

				372.75		0.7048984

				372.77		0.7048984

				372.79		0.7048984

				372.82		0.7048984

				372.84		0.7048984

				372.86		0.7048984

				372.88		0.6989247

				372.9		0.6989247

				372.92		0.6989247

				372.94		0.6989247

				372.96		0.7048984

				372.99		0.6989247

				373.01		0.6989247

				373.03		0.6989247

				373.05		0.6989247

				373.07		0.6989247

				373.09		0.6989247

				373.11		0.6989247

				373.13		0.6989247

				373.16		0.6989247

				373.18		0.6989247

				373.2		0.6989247

				373.22		0.6989247

				373.24		0.6989247

				373.26		0.6989247

				373.28		0.6989247

				373.31		0.7048984

				373.33		0.6989247

				373.35		0.7048984

				373.37		0.7048984

				373.39		0.7048984

				373.41		0.7048984

				373.43		0.7048984

				373.45		0.7048984

				373.48		0.7048984

				373.5		0.7048984

				373.52		0.7048984

				373.54		0.7048984

				373.56		0.7048984

				373.58		0.6989247

				373.6		0.7048984

				373.62		0.7048984

				373.65		0.7048984

				373.67		0.7048984

				373.69		0.6989247

				373.71		0.6989247

				373.73		0.6989247

				373.75		0.6989247

				373.77		0.6989247

				373.79		0.6989247

				373.82		0.6989247

				373.84		0.6989247

				373.86		0.6989247

				373.88		0.6989247

				373.9		0.6989247

				373.92		0.6989247

				373.94		0.6989247

				373.96		0.6989247

				373.99		0.6989247

				374.01		0.6989247

				374.03		0.6989247

				374.05		0.6989247

				374.07		0.6989247

				374.09		0.6989247

				374.11		0.6989247

				374.13		0.6989247

				374.16		0.6989247

				374.18		0.692951

				374.2		0.692951

				374.22		0.6989247

				374.24		0.6989247

				374.26		0.6989247

				374.28		0.6989247

				374.3		0.6989247

				374.33		0.6989247

				374.35		0.6989247

				374.37		0.6989247

				374.39		0.6989247

				374.41		0.6989247

				374.43		0.6989247

				374.45		0.6989247

				374.47		0.6989247

				374.5		0.692951

				374.52		0.692951

				374.54		0.692951

				374.56		0.692951

				374.58		0.692951

				374.6		0.692951

				374.62		0.692951

				374.64		0.692951

				374.67		0.692951

				374.69		0.692951

				374.71		0.692951

				374.73		0.692951

				374.75		0.692951

				374.77		0.692951

				374.79		0.692951

				374.81		0.692951

				374.84		0.692951

				374.86		0.692951

				374.88		0.692951

				374.9		0.6989247

				374.92		0.6989247

				374.94		0.6989247

				374.96		0.6989247

				374.98		0.6989247

				375.01		0.6989247

				375.03		0.6989247

				375.05		0.6989247

				375.07		0.6989247

				375.09		0.6989247

				375.11		0.6989247

				375.13		0.6989247

				375.15		0.6989247

				375.18		0.6989247

				375.2		0.6989247

				375.22		0.6989247

				375.24		0.6989247

				375.26		0.692951

				375.28		0.692951

				375.3		0.692951

				375.33		0.692951

				375.35		0.692951

				375.37		0.692951

				375.39		0.692951

				375.41		0.692951

				375.43		0.692951

				375.45		0.692951

				375.47		0.692951

				375.5		0.692951

				375.52		0.692951

				375.54		0.692951

				375.56		0.692951

				375.58		0.692951

				375.6		0.692951

				375.62		0.692951

				375.64		0.692951

				375.67		0.692951

				375.69		0.692951

				375.71		0.692951

				375.73		0.692951

				375.75		0.692951

				375.77		0.692951

				375.79		0.692951

				375.81		0.692951

				375.84		0.692951

				375.86		0.692951

				375.88		0.6989247

				375.9		0.692951

				375.92		0.6989247

				375.94		0.692951

				375.96		0.6989247

				375.98		0.692951

				376.01		0.6989247

				376.03		0.6989247

				376.05		0.6989247

				376.07		0.6989247

				376.09		0.6989247

				376.11		0.6989247

				376.13		0.6989247

				376.15		0.6989247

				376.18		0.6989247

				376.2		0.6989247

				376.22		0.6989247

				376.24		0.6989247

				376.26		0.6989247

				376.28		0.6989247

				376.3		0.6989247

				376.32		0.6989247

				376.35		0.6989247

				376.37		0.6989247

				376.39		0.6989247

				376.41		0.6989247

				376.43		0.7048984

				376.45		0.6989247

				376.47		0.7048984

				376.49		0.7048984

				376.52		0.7048984

				376.54		0.7048984

				376.56		0.7048984

				376.58		0.7048984

				376.6		0.7048984

				376.62		0.7048984

				376.64		0.7048984

				376.66		0.7048984

				376.69		0.7048984

				376.71		0.7048984

				376.73		0.7048984

				376.75		0.7048984

				376.77		0.7048984

				376.79		0.7048984

				376.81		0.7048984

				376.83		0.7048984

				376.86		0.7048984

				376.88		0.7048984

				376.9		0.7048984

				376.92		0.7048984

				376.94		0.7048984

				376.96		0.7048984

				376.98		0.7048984

				377.01		0.7048984

				377.03		0.7048984

				377.05		0.7048984

				377.07		0.7048984

				377.09		0.7048984

				377.11		0.7108722

				377.13		0.7048984

				377.15		0.7048984

				377.18		0.7108722

				377.2		0.7108722

				377.22		0.7108722

				377.24		0.7108722

				377.26		0.7108722

				377.28		0.7108722

				377.3		0.7108722

				377.32		0.7108722

				377.35		0.7108722

				377.37		0.7108722

				377.39		0.7108722

				377.41		0.7108722

				377.43		0.7108722

				377.45		0.7108722

				377.47		0.7108722

				377.49		0.7108722

				377.52		0.7108722

				377.54		0.7108722

				377.56		0.7108722

				377.58		0.7108722

				377.6		0.7108722

				377.62		0.7108722

				377.64		0.7108722

				377.66		0.7108722

				377.69		0.7108722

				377.71		0.7108722

				377.73		0.7108722

				377.75		0.7108722

				377.77		0.7108722

				377.79		0.7108722

				377.81		0.7108722

				377.83		0.7108722

				377.86		0.7108722

				377.88		0.7108722

				377.9		0.7108722

				377.92		0.7108722

				377.94		0.7108722

				377.96		0.7168459

				377.98		0.7108722

				378		0.7168459

				378.03		0.7168459

				378.05		0.7168459

				378.07		0.7168459

				378.09		0.7168459

				378.11		0.7108722

				378.13		0.7108722

				378.15		0.7108722

				378.17		0.7108722

				378.2		0.7108722

				378.22		0.7108722

				378.24		0.7108722

				378.26		0.7108722

				378.28		0.7108722

				378.3		0.7108722

				378.32		0.7108722

				378.34		0.7108722

				378.37		0.7108722

				378.39		0.7108722

				378.41		0.7108722

				378.43		0.7108722

				378.45		0.7108722

				378.47		0.7108722

				378.49		0.7108722

				378.51		0.7108722

				378.54		0.7108722

				378.56		0.7108722

				378.58		0.7108722

				378.6		0.7108722

				378.62		0.7108722

				378.64		0.7108722

				378.66		0.7108722

				378.68		0.7108722

				378.71		0.7108722

				378.73		0.7108722

				378.75		0.7108722

				378.77		0.7108722

				378.79		0.7108722

				378.81		0.7108722

				378.83		0.7108722

				378.85		0.7108722

				378.88		0.7048984

				378.9		0.7048984

				378.92		0.7108722

				378.94		0.7048984

				378.96		0.7048984

				378.98		0.7108722

				379		0.7048984

				379.02		0.7108722

				379.05		0.7108722

				379.07		0.7108722

				379.09		0.7048984

				379.11		0.7048984

				379.13		0.7048984

				379.15		0.7048984

				379.17		0.7048984

				379.19		0.7048984

				379.22		0.7048984

				379.24		0.7048984

				379.26		0.7048984

				379.28		0.7048984

				379.3		0.7048984

				379.32		0.7048984

				379.34		0.7048984

				379.36		0.7048984

				379.39		0.7048984

				379.41		0.7048984

				379.43		0.7048984

				379.45		0.7048984

				379.47		0.7048984

				379.49		0.7048984

				379.51		0.7048984

				379.53		0.7048984

				379.56		0.7048984

				379.58		0.7048984

				379.6		0.7048984

				379.62		0.7048984

				379.64		0.7048984

				379.66		0.7048984

				379.68		0.7048984

				379.7		0.7048984

				379.73		0.7048984

				379.75		0.7048984

				379.77		0.7048984

				379.79		0.7048984

				379.81		0.7048984

				379.83		0.7048984

				379.85		0.7048984

				379.87		0.7048984

				379.9		0.7048984

				379.92		0.7048984

				379.94		0.7048984

				379.96		0.7048984

				379.98		0.7048984

				380		0.7048984

				380.02		0.7048984

				380.04		0.7048984

				380.07		0.7048984

				380.09		0.7048984

				380.11		0.7048984

				380.13		0.7048984

				380.15		0.7048984

				380.17		0.7048984

				380.19		0.7048984

				380.21		0.7048984

				380.24		0.7048984

				380.26		0.7048984

				380.28		0.7048984

				380.3		0.7048984

				380.32		0.7048984

				380.34		0.7048984

				380.36		0.7048984

				380.38		0.7048984

				380.41		0.7048984

				380.43		0.7048984

				380.45		0.7048984

				380.47		0.7048984

				380.49		0.7048984

				380.51		0.7048984

				380.53		0.7048984

				380.55		0.7048984

				380.58		0.7048984

				380.6		0.7048984

				380.62		0.7048984

				380.64		0.7048984

				380.66		0.7048984

				380.68		0.7048984

				380.7		0.7048984

				380.72		0.7048984

				380.75		0.7048984

				380.77		0.7048984

				380.79		0.7048984

				380.81		0.7048984

				380.83		0.7048984

				380.85		0.7048984

				380.87		0.7048984

				380.89		0.7048984

				380.91		0.7048984

				380.94		0.7048984

				380.96		0.7048984

				380.98		0.7048984

				381		0.7048984

				381.02		0.7048984

				381.04		0.7048984

				381.06		0.7048984

				381.08		0.7048984

				381.11		0.7048984

				381.13		0.7048984

				381.15		0.7048984

				381.17		0.7048984

				381.19		0.7048984

				381.21		0.7048984

				381.23		0.7048984

				381.26		0.7048984

				381.28		0.7048984

				381.3		0.7048984

				381.32		0.7048984

				381.34		0.7048984

				381.36		0.7048984

				381.38		0.7048984

				381.4		0.7048984

				381.43		0.7048984

				381.45		0.7048984

				381.47		0.7048984

				381.49		0.7048984

				381.51		0.7048984

				381.53		0.7048984

				381.55		0.7048984

				381.57		0.7048984

				381.6		0.7048984

				381.62		0.7048984

				381.64		0.7048984

				381.66		0.6989247

				381.68		0.6989247

				381.7		0.6989247

				381.72		0.6989247

				381.74		0.6989247

				381.77		0.6989247

				381.79		0.6989247

				381.81		0.6989247

				381.83		0.6989247

				381.85		0.6989247

				381.87		0.6989247

				381.89		0.6989247

				381.91		0.6989247

				381.94		0.6989247

				381.96		0.6989247

				381.98		0.6989247

				382		0.6989247

				382.02		0.6989247

				382.04		0.6989247

				382.06		0.6989247

				382.08		0.6989247

				382.11		0.6989247

				382.13		0.6989247

				382.15		0.6989247

				382.17		0.6989247

				382.19		0.6989247

				382.21		0.692951

				382.23		0.692951

				382.25		0.692951

				382.28		0.692951

				382.3		0.692951

				382.32		0.692951

				382.34		0.692951

				382.36		0.692951

				382.38		0.692951

				382.4		0.692951

				382.42		0.692951

				382.44		0.692951

				382.47		0.692951

				382.49		0.692951

				382.51		0.692951

				382.53		0.692951

				382.55		0.692951

				382.57		0.692951

				382.59		0.692951

				382.61		0.692951

				382.64		0.692951

				382.66		0.692951

				382.68		0.692951

				382.7		0.692951

				382.72		0.692951

				382.74		0.692951

				382.76		0.692951

				382.78		0.692951

				382.81		0.692951

				382.83		0.692951

				382.85		0.692951

				382.87		0.692951

				382.89		0.692951

				382.91		0.692951

				382.93		0.692951

				382.95		0.692951

				382.98		0.692951

				383		0.692951

				383.02		0.692951

				383.04		0.692951

				383.06		0.692951

				383.08		0.692951

				383.1		0.692951

				383.12		0.692951

				383.15		0.692951

				383.17		0.692951

				383.19		0.692951

				383.21		0.692951

				383.23		0.692951

				383.25		0.692951

				383.27		0.692951

				383.29		0.692951

				383.32		0.692951

				383.34		0.692951

				383.36		0.692951

				383.38		0.692951

				383.4		0.692951

				383.42		0.692951

				383.44		0.692951

				383.46		0.692951

				383.49		0.692951

				383.51		0.692951

				383.53		0.692951

				383.55		0.692951

				383.57		0.692951

				383.59		0.692951

				383.61		0.692951

				383.63		0.692951

				383.65		0.692951

				383.68		0.692951

				383.7		0.692951

				383.72		0.692951

				383.74		0.692951

				383.76		0.692951

				383.78		0.692951

				383.8		0.692951

				383.82		0.692951

				383.85		0.692951

				383.87		0.692951

				383.89		0.692951

				383.91		0.6989247

				383.93		0.692951

				383.95		0.6989247

				383.97		0.6989247

				383.99		0.6989247

				384.02		0.6989247

				384.04		0.6989247

				384.06		0.6989247

				384.08		0.6989247

				384.1		0.6989247

				384.12		0.6989247

				384.14		0.6989247

				384.16		0.6989247

				384.19		0.6989247

				384.21		0.6989247

				384.23		0.6989247

				384.25		0.6989247

				384.27		0.6989247

				384.29		0.6989247

				384.31		0.6989247

				384.33		0.6989247

				384.35		0.6989247

				384.38		0.6989247

				384.4		0.6989247

				384.42		0.6989247

				384.44		0.6989247

				384.46		0.6989247

				384.48		0.6989247

				384.5		0.6989247

				384.52		0.6989247

				384.55		0.6989247

				384.57		0.6989247

				384.59		0.6989247

				384.61		0.6989247

				384.63		0.6989247

				384.65		0.6989247

				384.67		0.6989247

				384.69		0.6989247

				384.72		0.6989247

				384.74		0.6989247

				384.76		0.6989247

				384.78		0.6989247

				384.8		0.6989247

				384.82		0.6989247

				384.84		0.6989247

				384.86		0.6989247

				384.88		0.6989247

				384.91		0.6989247

				384.93		0.6989247

				384.95		0.6989247

				384.97		0.6989247

				384.99		0.6989247

				385.01		0.6989247

				385.03		0.6989247

				385.05		0.6989247

				385.08		0.6989247

				385.1		0.6989247

				385.12		0.6989247

				385.14		0.6989247

				385.16		0.6989247

				385.18		0.6989247

				385.2		0.6989247

				385.22		0.7048984

				385.25		0.7048984

				385.27		0.7048984

				385.29		0.7048984

				385.31		0.7048984

				385.33		0.7048984

				385.35		0.7048984

				385.37		0.7048984

				385.39		0.7048984

				385.42		0.7048984

				385.44		0.7048984

				385.46		0.7048984

				385.48		0.7048984

				385.5		0.6989247

				385.52		0.7048984

				385.54		0.6989247

				385.56		0.6989247

				385.58		0.7048984

				385.61		0.6989247

				385.63		0.6989247

				385.65		0.6989247

				385.67		0.6989247

				385.69		0.6989247

				385.71		0.6989247

				385.73		0.6989247

				385.75		0.6989247

				385.78		0.6989247

				385.8		0.6989247

				385.82		0.6989247

				385.84		0.6989247

				385.86		0.6989247

				385.88		0.6989247

				385.9		0.6989247

				385.92		0.6989247

				385.95		0.6989247

				385.97		0.6989247

				385.99		0.6989247

				386.01		0.6989247

				386.03		0.6989247

				386.05		0.6989247

				386.07		0.6989247

				386.09		0.6989247

				386.12		0.6989247

				386.14		0.6989247

				386.16		0.6989247

				386.18		0.6989247

				386.2		0.6989247

				386.22		0.6989247

				386.24		0.692951

				386.26		0.6989247

				386.29		0.6989247

				386.31		0.6989247

				386.33		0.6989247

				386.35		0.6989247

				386.37		0.6989247

				386.39		0.6989247

				386.41		0.6989247

				386.43		0.6989247

				386.46		0.6989247

				386.48		0.692951

				386.5		0.692951

				386.52		0.692951

				386.54		0.692951

				386.56		0.692951

				386.58		0.692951

				386.6		0.692951

				386.63		0.692951

				386.65		0.692951

				386.67		0.692951

				386.69		0.692951

				386.71		0.692951

				386.73		0.692951

				386.75		0.692951

				386.77		0.692951

				386.79		0.692951

				386.82		0.692951

				386.84		0.692951

				386.86		0.692951

				386.88		0.692951

				386.9		0.692951

				386.92		0.692951

				386.94		0.692951

				386.96		0.692951

				386.99		0.692951

				387.01		0.692951

				387.03		0.692951

				387.05		0.692951

				387.07		0.692951

				387.09		0.692951

				387.11		0.692951

				387.13		0.692951

				387.16		0.692951

				387.18		0.692951

				387.2		0.692951

				387.22		0.692951

				387.24		0.692951

				387.26		0.692951

				387.28		0.692951

				387.3		0.692951

				387.32		0.692951

				387.35		0.692951

				387.37		0.692951

				387.39		0.692951

				387.41		0.692951

				387.43		0.692951

				387.45		0.692951

				387.47		0.692951

				387.49		0.692951

				387.52		0.692951

				387.54		0.692951

				387.56		0.692951

				387.58		0.692951

				387.6		0.692951

				387.62		0.692951

				387.64		0.692951

				387.66		0.692951

				387.69		0.692951

				387.71		0.692951

				387.73		0.692951

				387.75		0.692951

				387.77		0.692951

				387.79		0.692951

				387.81		0.692951

				387.83		0.692951

				387.86		0.692951

				387.88		0.692951

				387.9		0.692951

				387.92		0.692951

				387.94		0.692951

				387.96		0.692951

				387.98		0.692951

				388		0.692951

				388.02		0.692951

				388.05		0.692951

				388.07		0.692951

				388.09		0.692951

				388.11		0.692951

				388.13		0.692951

				388.15		0.692951

				388.17		0.692951

				388.19		0.692951

				388.22		0.692951

				388.24		0.692951

				388.26		0.692951

				388.28		0.692951

				388.3		0.692951

				388.32		0.692951

				388.34		0.692951

				388.36		0.692951

				388.39		0.692951

				388.41		0.692951

				388.43		0.692951

				388.45		0.692951

				388.47		0.692951

				388.49		0.6989247

				388.51		0.692951

				388.53		0.6989247

				388.55		0.6989247

				388.58		0.6989247

				388.6		0.6989247

				388.62		0.6989247

				388.64		0.6989247

				388.66		0.6989247

				388.68		0.6989247

				388.7		0.6989247

				388.72		0.6989247

				388.75		0.6989247

				388.77		0.6989247

				388.79		0.6989247

				388.81		0.6989247

				388.83		0.6989247

				388.85		0.6989247

				388.87		0.6989247

				388.89		0.6989247

				388.92		0.6989247

				388.94		0.6989247

				388.96		0.6989247

				388.98		0.6989247

				389		0.6989247

				389.02		0.6989247

				389.04		0.6989247

				389.06		0.6989247

				389.08		0.6989247

				389.11		0.6989247

				389.13		0.6989247

				389.15		0.6989247

				389.17		0.6989247

				389.19		0.6989247

				389.21		0.6989247

				389.23		0.6989247

				389.25		0.6989247

				389.28		0.6989247

				389.3		0.6989247

				389.32		0.6989247

				389.34		0.6989247

				389.36		0.6989247

				389.38		0.6989247

				389.4		0.6989247

				389.42		0.6989247

				389.45		0.692951

				389.47		0.692951

				389.49		0.692951

				389.51		0.692951

				389.53		0.692951

				389.55		0.692951

				389.57		0.692951

				389.59		0.692951

				389.61		0.692951

				389.64		0.692951

				389.66		0.692951

				389.68		0.692951

				389.7		0.692951

				389.72		0.692951

				389.74		0.692951

				389.76		0.692951

				389.78		0.692951

				389.81		0.692951

				389.83		0.692951

				389.85		0.692951

				389.87		0.692951

				389.89		0.692951

				389.91		0.692951

				389.93		0.692951

				389.95		0.692951

				389.98		0.692951

				390		0.692951

				390.02		0.692951

				390.04		0.692951

				390.06		0.692951

				390.08		0.692951

				390.1		0.692951

				390.12		0.692951

				390.14		0.692951

				390.17		0.692951

				390.19		0.692951

				390.21		0.692951

				390.23		0.692951

				390.25		0.6869773

				390.27		0.692951

				390.29		0.692951

				390.31		0.692951

				390.34		0.692951

				390.36		0.692951

				390.38		0.692951

				390.4		0.6869773

				390.42		0.6869773

				390.44		0.6869773

				390.46		0.6869773

				390.48		0.6869773

				390.51		0.6869773

				390.53		0.6869773

				390.55		0.6869773

				390.57		0.6869773

				390.59		0.6869773

				390.61		0.6869773

				390.63		0.6869773

				390.65		0.6869773

				390.67		0.6869773

				390.7		0.6869773

				390.72		0.6869773

				390.74		0.6869773

				390.76		0.6869773

				390.78		0.6869773

				390.8		0.6810036

				390.82		0.6810036

				390.84		0.6869773

				390.87		0.6810036

				390.89		0.6810036

				390.91		0.6810036

				390.93		0.6810036

				390.95		0.6810036

				390.97		0.6869773

				390.99		0.6869773

				391.01		0.6869773

				391.03		0.6869773

				391.06		0.6869773

				391.08		0.6869773

				391.1		0.6869773

				391.12		0.6810036

				391.14		0.6810036

				391.16		0.6810036

				391.18		0.6810036

				391.2		0.6810036

				391.23		0.6869773

				391.25		0.6869773

				391.27		0.6869773

				391.29		0.6869773

				391.31		0.6869773

				391.33		0.6869773

				391.35		0.6869773

				391.37		0.6869773

				391.39		0.6869773

				391.42		0.6869773

				391.44		0.6869773

				391.46		0.6869773

				391.48		0.6869773

				391.5		0.6869773

				391.52		0.6869773

				391.54		0.6869773

				391.56		0.6869773

				391.59		0.6869773

				391.61		0.6869773

				391.63		0.6869773

				391.65		0.6869773

				391.67		0.6869773

				391.69		0.6869773

				391.71		0.6869773

				391.73		0.6869773

				391.75		0.6869773

				391.78		0.6869773

				391.8		0.692951

				391.82		0.692951

				391.84		0.692951

		Results:

		Onset		X1		192.14		°C

				Y1		93.612		%

				X2		249.26		°C

				Y2		10.579		%

				Onset X		229.12		°C

				Onset Y		80.357		%
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RT54-0.2MWCNT.xlsx
Sheet1

		Method Filename:		C:\Program Files (x86)\PerkinElmer\Pyris\data\Anas\21052024\RT54-MWCNT 0.2.t6d

		Sample ID:		RT54-MWCNT 0.2

		Step:		1

		Data		Sample Temperature (°C)		Weight % (%)

				30.09		99.9948

				30.09		99.9948

				30.09		99.9948

				30.09		99.98959

				30.09		99.9948

				30.09		99.98959

				30.09		99.9948

				30.09		99.9948

				30.09		99.9948

				30.09		99.98959

				30.09		99.98959

				30.09		99.98959

				30.09		99.98959

				30.09		99.98959

				30.09		99.98959

				30.09		99.98959

				30.09		99.98959

				30.09		99.9948

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98439

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.98959

				30.08		99.9948

				30.08		99.9948

				30.08		99.9948

				30.08		99.9948

				30.08		99.9948

				30.08		99.9948

				30.08		99.9948

				30.08		99.9948

				30.08		99.9948

				30.08		99.9948

				30.08		99.9948

				30.08		99.9948

				30.08		99.9948

				30.08		99.9948

				30.08		99.9948

				30.08		100

				30.08		99.9948

				30.08		100

				30.08		100

				30.08		100

				30.08		100

				30.08		100

				30.08		100

				30.08		100

				30.08		100

				30.08		100

				30.08		100

				30.08		100.0052

				30.08		100.0052

				30.08		100.0052

				30.08		100.0052

				30.08		100.0052

				30.08		100.0052

				30.08		100.0052

				30.08		100.0052

				30.08		100.0052

				30.08		100.0052

				30.08		100.0052

				30.08		100.0052

				30.08		100.0052

				30.08		100.0052

				30.08		100.0104

				30.08		100.0104

				30.08		100.0104

				30.09		100.0104

				30.09		100.0104

				30.09		100.0052

				30.09		100.0104

				30.09		100.0104

				30.09		100.0104

				30.09		100.0104

				30.09		100.0104

				30.09		100.0104

				30.09		100.0104

				30.09		100.0104

				30.09		100.0104

				30.1		100.0104

				30.1		100.0104

				30.1		100.0104

				30.1		100.0156

				30.1		100.0156

				30.1		100.0156

				30.1		100.0156

				30.1		100.0156

				30.1		100.0156

				30.11		100.0156

				30.11		100.0156

				30.11		100.0156

				30.11		100.0156

				30.11		100.0208

				30.11		100.0208

				30.12		100.0208

				30.12		100.0208

				30.12		100.0208

				30.12		100.0208

				30.12		100.0208

				30.12		100.0208

				30.13		100.0208

				30.13		100.0208

				30.13		100.0208

				30.13		100.0208

				30.13		100.0208

				30.14		100.0208

				30.14		100.0208

				30.14		100.0208

				30.14		100.0208

				30.14		100.026

				30.15		100.026

				30.15		100.026

				30.15		100.026

				30.15		100.026

				30.16		100.026

				30.16		100.026

				30.16		100.0312

				30.16		100.0312

				30.17		100.0312

				30.17		100.0312

				30.17		100.0312

				30.17		100.0312

				30.18		100.0312

				30.18		100.0312

				30.18		100.0312

				30.19		100.0312

				30.19		100.0312

				30.19		100.0312

				30.19		100.0364

				30.2		100.0364

				30.2		100.0364

				30.2		100.0364

				30.21		100.0364

				30.21		100.0364

				30.21		100.0364

				30.22		100.0364

				30.22		100.0364

				30.22		100.0364

				30.23		100.0416

				30.23		100.0416

				30.24		100.0416

				30.24		100.0416

				30.24		100.0416

				30.25		100.0416

				30.25		100.0416

				30.25		100.0416

				30.26		100.0416

				30.26		100.0416

				30.27		100.0416

				30.27		100.0468

				30.27		100.0468

				30.28		100.0468

				30.28		100.0468

				30.29		100.0468

				30.29		100.0468

				30.29		100.0468

				30.3		100.0468

				30.3		100.0468

				30.31		100.0468

				30.31		100.0468

				30.32		100.052

				30.32		100.0468

				30.32		100.0468

				30.33		100.052

				30.33		100.052

				30.34		100.052

				30.34		100.052

				30.35		100.052

				30.35		100.052

				30.36		100.052

				30.36		100.052

				30.37		100.052

				30.37		100.0572

				30.38		100.052

				30.38		100.0572

				30.39		100.0572

				30.39		100.0572

				30.4		100.0572

				30.4		100.0572

				30.41		100.0572

				30.41		100.0572

				30.42		100.0572

				30.42		100.0572

				30.43		100.0624

				30.43		100.0624

				30.44		100.0624

				30.44		100.0624

				30.45		100.0624

				30.46		100.0624

				30.46		100.0624

				30.47		100.0624

				30.47		100.0624

				30.48		100.0624

				30.48		100.0676

				30.49		100.0676

				30.49		100.0676

				30.5		100.0676

				30.51		100.0676

				30.51		100.0676

				30.52		100.0676

				30.52		100.0676

				30.53		100.0676

				30.54		100.0676

				30.54		100.0676

				30.55		100.0676

				30.55		100.0676

				30.56		100.0676

				30.57		100.0729

				30.57		100.0676

				30.58		100.0729

				30.58		100.0729

				30.59		100.0729

				30.6		100.0729

				30.6		100.0729

				30.61		100.0729

				30.62		100.0729

				30.62		100.0729

				30.63		100.0781

				30.64		100.0729

				30.64		100.0781

				30.65		100.0729

				30.65		100.0781

				30.66		100.0729

				30.67		100.0729

				30.67		100.0781

				30.68		100.0781

				30.69		100.0781

				30.69		100.0781

				30.7		100.0781

				30.71		100.0781

				30.72		100.0781

				30.72		100.0781

				30.73		100.0833

				30.74		100.0833

				30.74		100.0833

				30.75		100.0833

				30.76		100.0833

				30.76		100.0833

				30.77		100.0833

				30.78		100.0833

				30.79		100.0833

				30.79		100.0833

				30.8		100.0833

				30.81		100.0833

				30.81		100.0833

				30.82		100.0833

				30.83		100.0833

				30.84		100.0833

				30.84		100.0833

				30.85		100.0833

				30.86		100.0833

				30.87		100.0833

				30.87		100.0833

				30.88		100.0885

				30.89		100.0885

				30.9		100.0833

				30.9		100.0885

				30.91		100.0885

				30.92		100.0885

				30.93		100.0885

				30.93		100.0885

				30.94		100.0937

				30.95		100.0885

				30.96		100.0885

				30.96		100.0885

				30.97		100.0885

				30.98		100.0937

				30.99		100.0937

				31		100.0937

				31		100.0937

				31.01		100.0937

				31.02		100.0937

				31.03		100.0937

				31.04		100.0937

				31.04		100.0937

				31.05		100.0937

				31.06		100.0937

				31.07		100.0937

				31.08		100.0937

				31.08		100.0937

				31.09		100.0937

				31.1		100.0937

				31.11		100.0937

				31.12		100.0937

				31.13		100.0937

				31.13		100.0937

				31.14		100.0937

				31.15		100.0937

				31.16		100.0937

				31.17		100.0937

				31.18		100.0937

				31.18		100.0937

				31.19		100.0937

				31.2		100.0937

				31.21		100.0937

				31.22		100.0937

				31.23		100.0937

				31.24		100.0937

				31.24		100.0937

				31.25		100.0937

				31.26		100.0937

				31.27		100.0937

				31.28		100.0937

				31.29		100.0937

				31.3		100.0937

				31.31		100.0937

				31.31		100.0937

				31.32		100.0937

				31.33		100.0989

				31.34		100.0937

				31.35		100.0937

				31.36		100.0937

				31.37		100.0937

				31.38		100.0937

				31.39		100.0989

				31.39		100.0989

				31.4		100.0937

				31.41		100.0989

				31.42		100.0937

				31.43		100.0937

				31.44		100.0937

				31.45		100.0989

				31.46		100.0989

				31.47		100.0989

				31.48		100.0989

				31.49		100.0989

				31.49		100.0989

				31.5		100.0989

				31.51		100.0989

				31.52		100.0989

				31.53		100.0989

				31.54		100.0989

				31.55		100.0989

				31.56		100.0989

				31.57		100.0989

				31.58		100.0989

				31.59		100.0989

				31.6		100.0989

				31.61		100.1041

				31.62		100.1041

				31.63		100.1041

				31.64		100.1041

				31.65		100.1041

				31.66		100.1041

				31.67		100.1041

				31.67		100.1041

				31.68		100.1041

				31.69		100.1041

				31.7		100.1093

				31.71		100.1093

				31.72		100.1093

				31.73		100.1093

				31.74		100.1093

				31.75		100.1093

				31.76		100.1093

				31.77		100.1093

				31.78		100.1093

				31.79		100.1093

				31.8		100.1093

				31.81		100.1041

				31.82		100.1093

				31.83		100.1093

				31.84		100.1093

				31.85		100.1093

				31.86		100.1093

				31.87		100.1093

				31.88		100.1093

				31.89		100.1093

				31.9		100.1093

				31.91		100.1093

				31.92		100.1093

				31.93		100.1093

				31.94		100.1093

				31.95		100.1093

				31.96		100.1145

				31.98		100.1145

				31.99		100.1145

				32		100.1145

				32.01		100.1145

				32.02		100.1145

				32.03		100.1145

				32.04		100.1145

				32.05		100.1145

				32.06		100.1145

				32.07		100.1145

				32.08		100.1145

				32.09		100.1197

				32.1		100.1197

				32.11		100.1197

				32.12		100.1197

				32.13		100.1197

				32.14		100.1197

				32.15		100.1197

				32.16		100.1197

				32.17		100.1197

				32.19		100.1197

				32.2		100.1197

				32.21		100.1197

				32.22		100.1249

				32.23		100.1249

				32.24		100.1249

				32.25		100.1249

				32.26		100.1249

				32.27		100.1249

				32.28		100.1249

				32.29		100.1249

				32.3		100.1249

				32.32		100.1249

				32.33		100.1249

				32.34		100.1249

				32.35		100.1249

				32.36		100.1301

				32.37		100.1301

				32.38		100.1301

				32.39		100.1301

				32.4		100.1301

				32.41		100.1301

				32.43		100.1301

				32.44		100.1301

				32.45		100.1301

				32.46		100.1301

				32.47		100.1301

				32.48		100.1301

				32.49		100.1301

				32.5		100.1301

				32.52		100.1301

				32.53		100.1353

				32.54		100.1353

				32.55		100.1353

				32.56		100.1353

				32.57		100.1353

				32.58		100.1353

				32.6		100.1353

				32.61		100.1353

				32.62		100.1353

				32.63		100.1353

				32.64		100.1353

				32.65		100.1353

				32.66		100.1353

				32.68		100.1353

				32.69		100.1353

				32.7		100.1353

				32.71		100.1353

				32.72		100.1353

				32.73		100.1353

				32.75		100.1353

				32.76		100.1353

				32.77		100.1405

				32.78		100.1405

				32.79		100.1405

				32.8		100.1405

				32.82		100.1405

				32.83		100.1405

				32.84		100.1405

				32.85		100.1405

				32.86		100.1353

				32.88		100.1301

				32.89		100.1301

				32.9		100.1301

				32.91		100.1301

				32.92		100.1301

				32.93		100.1301

				32.95		100.1301

				32.96		100.1301

				32.97		100.1301

				32.98		100.1353

				32.99		100.1353

				33.01		100.1353

				33.02		100.1353

				33.03		100.1353

				33.04		100.1353

				33.06		100.1353

				33.07		100.1353

				33.08		100.1353

				33.09		100.1405

				33.1		100.1405

				33.12		100.1405

				33.13		100.1405

				33.14		100.1405

				33.15		100.1405

				33.17		100.1405

				33.18		100.1405

				33.19		100.1405

				33.2		100.1405

				33.21		100.1457

				33.23		100.1457

				33.24		100.1457

				33.25		100.1457

				33.26		100.1457

				33.28		100.1457

				33.29		100.1457

				33.3		100.1457

				33.31		100.1457

				33.33		100.1457

				33.34		100.1457

				33.35		100.1457

				33.36		100.1509

				33.38		100.1509

				33.39		100.1509

				33.4		100.1509

				33.41		100.1561

				33.43		100.1613

				33.44		100.1613

				33.45		100.1665

				33.47		100.1665

				33.48		100.1665

				33.49		100.1665

				33.5		100.1665

				33.52		100.1665

				33.53		100.1665

				33.54		100.1665

				33.55		100.1717

				33.57		100.1717

				33.58		100.1717

				33.59		100.1717

				33.61		100.1717

				33.62		100.1717

				33.63		100.1717

				33.64		100.1717

				33.66		100.1717

				33.67		100.1717

				33.68		100.1769

				33.7		100.1769

				33.71		100.1769

				33.72		100.1769

				33.74		100.1769

				33.75		100.1769

				33.76		100.1769

				33.77		100.1769

				33.79		100.1717

				33.8		100.1717

				33.81		100.1717

				33.83		100.1717

				33.84		100.1717

				33.85		100.1717

				33.87		100.1665

				33.88		100.1717

				33.89		100.1717

				33.91		100.1717

				33.92		100.1821

				33.93		100.1821

				33.95		100.1821

				33.96		100.1821

				33.97		100.1873

				33.99		100.1873

				34		100.1873

				34.01		100.1873

				34.03		100.1821

				34.04		100.1821

				34.05		100.1821

				34.07		100.1821

				34.08		100.1821

				34.09		100.1821

				34.11		100.1821

				34.12		100.1821

				34.13		100.1821

				34.15		100.1821

				34.16		100.1821

				34.17		100.1821

				34.19		100.1821

				34.2		100.1821

				34.22		100.1821

				34.23		100.1821

				34.24		100.1821

				34.26		100.1821

				34.27		100.1821

				34.28		100.1821

				34.3		100.1821

				34.31		100.1821

				34.32		100.1821

				34.34		100.1821

				34.35		100.1821

				34.37		100.1821

				34.38		100.1821

				34.39		100.1821

				34.41		100.1821

				34.42		100.1821

				34.44		100.1821

				34.45		100.1821

				34.46		100.1821

				34.48		100.1821

				34.49		100.1821

				34.5		100.1821

				34.52		100.1821

				34.53		100.1821

				34.55		100.1821

				34.56		100.1821

				34.57		100.1821

				34.59		100.1821

				34.6		100.1821

				34.62		100.1821

				34.63		100.1821

				34.64		100.1821

				34.66		100.1821

				34.67		100.1821

				34.69		100.1873

				34.7		100.1821

				34.71		100.1821

				34.73		100.1821

				34.74		100.1769

				34.76		100.1769

				34.77		100.1769

				34.79		100.1717

				34.8		100.1717

				34.81		100.1717

				34.83		100.1717

				34.84		100.1717

				34.86		100.1717

				34.87		100.1769

				34.88		100.1717

				34.9		100.1717

				34.91		100.1769

				34.93		100.1769

				34.94		100.1769

				34.96		100.1769

				34.97		100.1769

				34.99		100.1769

				35		100.1769

				35.01		100.1769

				35.03		100.1769

				35.04		100.1769

				35.06		100.1769

				35.07		100.1769

				35.09		100.1769

				35.1		100.1769

				35.11		100.1769

				35.13		100.1769

				35.14		100.1769

				35.16		100.1769

				35.17		100.1769

				35.19		100.1769

				35.2		100.1769

				35.22		100.1769

				35.23		100.1769

				35.25		100.1769

				35.26		100.1769

				35.27		100.1769

				35.29		100.1769

				35.3		100.1769

				35.32		100.1821

				35.33		100.1821

				35.35		100.1769

				35.36		100.1821

				35.38		100.1821

				35.39		100.1821

				35.41		100.1821

				35.42		100.1821

				35.44		100.1821

				35.45		100.1821

				35.47		100.1821

				35.48		100.1821

				35.5		100.1821

				35.51		100.1821

				35.53		100.1821

				35.54		100.1821

				35.55		100.1821

				35.57		100.1821

				35.58		100.1821

				35.6		100.1821

				35.61		100.1821

				35.63		100.1821

				35.64		100.1821

				35.66		100.1821

				35.67		100.1821

				35.69		100.1821

				35.7		100.1821

				35.72		100.1821

				35.73		100.1821

				35.75		100.1821

				35.76		100.1821

				35.78		100.1821

				35.79		100.1821

				35.81		100.1821

				35.82		100.1821

				35.84		100.1821

				35.85		100.1821

				35.87		100.1821

				35.89		100.1821

				35.9		100.1821

				35.92		100.1821

				35.93		100.1821

				35.95		100.1821

				35.96		100.1821

				35.98		100.1821

				35.99		100.1821

				36.01		100.1821

				36.02		100.1821

				36.04		100.1821

				36.05		100.1821

				36.07		100.1873

				36.08		100.1821

				36.1		100.1873

				36.11		100.1873

				36.13		100.1873

				36.14		100.1873

				36.16		100.1873

				36.17		100.1873

				36.19		100.1873

				36.21		100.1821

				36.22		100.1873

				36.24		100.1821

				36.25		100.1821

				36.27		100.1873

				36.28		100.1873

				36.3		100.1873

				36.31		100.1873

				36.33		100.1873

				36.34		100.1873

				36.36		100.1873

				36.37		100.1873

				36.39		100.1873

				36.41		100.1925

				36.42		100.1925

				36.44		100.1925

				36.45		100.1925

				36.47		100.1925

				36.48		100.1925

				36.5		100.1925

				36.51		100.1925

				36.53		100.1925

				36.55		100.1925

				36.56		100.1925

				36.58		100.1925

				36.59		100.1925

				36.61		100.1925

				36.62		100.1925

				36.64		100.1925

				36.66		100.1925

				36.67		100.1977

				36.69		100.1977

				36.7		100.1977

				36.72		100.1977

				36.73		100.1977

				36.75		100.1977

				36.77		100.1977

				36.78		100.1977

				36.8		100.1977

				36.81		100.1977

				36.83		100.1977

				36.84		100.1977

				36.86		100.1977

				36.88		100.1977

				36.89		100.1977

				36.91		100.1977

				36.92		100.1977

				36.94		100.1977

				36.96		100.1977

				36.97		100.1977

				36.99		100.1977

				37		100.1977

				37.02		100.1977

				37.03		100.1977

				37.05		100.1977

				37.07		100.2029

				37.08		100.2029

				37.1		100.2029

				37.11		100.2029

				37.13		100.2029

				37.15		100.2029

				37.16		100.2029

				37.18		100.2029

				37.19		100.2029

				37.21		100.2029

				37.23		100.2029

				37.24		100.2029

				37.26		100.2029

				37.27		100.2081

				37.29		100.2081

				37.31		100.2081

				37.32		100.2029

				37.34		100.2029

				37.36		100.2029

				37.37		100.2081

				37.39		100.2081

				37.4		100.2081

				37.42		100.2081

				37.44		100.2081

				37.45		100.2081

				37.47		100.2081

				37.48		100.2081

				37.5		100.2134

				37.52		100.2134

				37.53		100.2134

				37.55		100.2134

				37.57		100.2081

				37.58		100.2081

				37.6		100.2081

				37.61		100.2081

				37.63		100.2081

				37.65		100.2081

				37.66		100.2081

				37.68		100.2081

				37.7		100.2081

				37.71		100.2081

				37.73		100.2081

				37.75		100.2081

				37.76		100.2081

				37.78		100.2134

				37.79		100.2134

				37.81		100.2134

				37.83		100.2134

				37.84		100.2134

				37.86		100.2134

				37.88		100.2134

				37.89		100.2134

				37.91		100.2134

				37.93		100.2134

				37.94		100.2134

				37.96		100.2134

				37.97		100.2134

				37.99		100.2134

				38.01		100.2134

				38.02		100.2134

				38.04		100.2134

				38.06		100.2134

				38.07		100.2134

				38.09		100.2134

				38.11		100.2081

				38.12		100.2081

				38.14		100.2029

				38.16		100.2029

				38.17		100.2029

				38.19		100.2029

				38.21		100.2029

				38.22		100.2029

				38.24		100.2029

				38.26		100.2081

				38.27		100.2081

				38.29		100.2081

				38.31		100.2081

				38.32		100.2134

				38.34		100.2134

				38.36		100.2134

				38.37		100.2134

				38.39		100.2134

				38.41		100.2134

				38.42		100.2134

				38.44		100.2134

				38.46		100.2134

				38.47		100.2134

				38.49		100.2134

				38.51		100.2134

				38.52		100.2134

				38.54		100.2134

				38.56		100.2134

				38.57		100.2134

				38.59		100.2134

				38.61		100.2134

				38.62		100.2134

				38.64		100.2134

				38.66		100.2134

				38.67		100.2134

				38.69		100.2134

				38.71		100.2134

				38.73		100.2134

				38.74		100.2134

				38.76		100.2134

				38.78		100.2134

				38.79		100.2134

				38.81		100.2134

				38.83		100.2134

				38.84		100.2134

				38.86		100.2134

				38.88		100.2134

				38.89		100.2186

				38.91		100.2134

				38.93		100.2134

				38.95		100.2134

				38.96		100.2186

				38.98		100.2186

				39		100.2186

				39.01		100.2186

				39.03		100.2134

				39.05		100.2134

				39.06		100.2134

				39.08		100.2134

				39.1		100.2134

				39.12		100.2134

				39.13		100.2134

				39.15		100.2134

				39.17		100.2134

				39.18		100.2134

				39.2		100.2134

				39.22		100.2134

				39.24		100.2186

				39.25		100.2186

				39.27		100.2186

				39.29		100.2186

				39.3		100.2186

				39.32		100.2186

				39.34		100.2186

				39.36		100.2186

				39.37		100.2186

				39.39		100.2186

				39.41		100.2186

				39.42		100.2186

				39.44		100.2186

				39.46		100.2186

				39.48		100.2186

				39.49		100.2186

				39.51		100.2186

				39.53		100.2186

				39.54		100.2186

				39.56		100.2186

				39.58		100.2186

				39.6		100.2134

				39.61		100.2186

				39.63		100.2186

				39.65		100.2186

				39.67		100.2186

				39.68		100.2134

				39.7		100.2134

				39.72		100.2134

				39.73		100.2134

				39.75		100.2134

				39.77		100.2134

				39.79		100.2186

				39.8		100.2186

				39.82		100.2238

				39.84		100.229

				39.86		100.229

				39.87		100.229

				39.89		100.229

				39.91		100.229

				39.93		100.2238

				39.94		100.2238

				39.96		100.2238

				39.98		100.2238

				40		100.2186

				40.01		100.2186

				40.03		100.2186

				40.05		100.2186

				40.07		100.2186

				40.08		100.2186

				40.1		100.2186

				40.12		100.2134

				40.14		100.2134

				40.15		100.2134

				40.17		100.2134

				40.19		100.2134

				40.21		100.2134

				40.22		100.2134

				40.24		100.2134

				40.26		100.2134

				40.28		100.2134

				40.29		100.2134

				40.31		100.2134

				40.33		100.2134

				40.35		100.2134

				40.36		100.2134

				40.38		100.2134

				40.4		100.2134

				40.42		100.2134

				40.43		100.2134

				40.45		100.2186

				40.47		100.2134

				40.49		100.2134

				40.51		100.2134

				40.52		100.2134

				40.54		100.2134

				40.56		100.2134

				40.58		100.2134

				40.59		100.2134

				40.61		100.2134

				40.63		100.2186

				40.65		100.2186

				40.66		100.2186

				40.68		100.2186

				40.7		100.2186

				40.72		100.2186

				40.74		100.2186

				40.75		100.2238

				40.77		100.2238

				40.79		100.2238

				40.81		100.2238

				40.82		100.2238

				40.84		100.2238

				40.86		100.2186

				40.88		100.2238

				40.9		100.2238

				40.91		100.2238

				40.93		100.2238

				40.95		100.2238

				40.97		100.2238

				40.98		100.2238

				41		100.2238

				41.02		100.2238

				41.04		100.2238

				41.06		100.2238

				41.07		100.2238

				41.09		100.2238

				41.11		100.2238

				41.13		100.2238

				41.15		100.2238

				41.16		100.2238

				41.18		100.2238

				41.2		100.2238

				41.22		100.2238

				41.24		100.2238

				41.25		100.2238

				41.27		100.229

				41.29		100.229

				41.31		100.229

				41.32		100.229

				41.34		100.229

				41.36		100.229

				41.38		100.229

				41.4		100.229

				41.41		100.229

				41.43		100.229

				41.45		100.229

				41.47		100.229

				41.49		100.229

				41.5		100.229

				41.52		100.2342

				41.54		100.229

				41.56		100.2342

				41.58		100.2342

				41.59		100.2342

				41.61		100.2342

				41.63		100.2342

				41.65		100.2342

				41.67		100.2342

				41.69		100.2342

				41.7		100.2342

				41.72		100.2342

				41.74		100.2342

				41.76		100.2342

				41.78		100.2342

				41.79		100.2342

				41.81		100.2342

				41.83		100.2342

				41.85		100.2342

				41.87		100.2394

				41.88		100.2394

				41.9		100.2394

				41.92		100.2394

				41.94		100.2394

				41.96		100.2394

				41.98		100.2394

				41.99		100.2446

				42.01		100.2446

				42.03		100.2446

				42.05		100.2446

				42.07		100.2446

				42.08		100.2446

				42.1		100.2446

				42.12		100.2446

				42.14		100.2446

				42.16		100.2446

				42.18		100.2446

				42.19		100.2446

				42.21		100.2446

				42.23		100.2446

				42.25		100.2498

				42.27		100.2446

				42.28		100.2446

				42.3		100.2498

				42.32		100.2446

				42.34		100.2498

				42.36		100.2498

				42.38		100.2498

				42.39		100.2498

				42.41		100.2446

				42.43		100.2446

				42.45		100.2446

				42.47		100.2446

				42.49		100.2446

				42.5		100.2446

				42.52		100.2446

				42.54		100.2446

				42.56		100.2446

				42.58		100.2446

				42.6		100.2446

				42.61		100.2446

				42.63		100.2446

				42.65		100.2446

				42.67		100.2446

				42.69		100.2498

				42.71		100.2498

				42.72		100.2498

				42.74		100.2498

				42.76		100.2498

				42.78		100.2498

				42.8		100.2498

				42.82		100.2498

				42.84		100.2498

				42.85		100.2498

				42.87		100.2498

				42.89		100.2498

				42.91		100.2498

				42.93		100.2498

				42.95		100.2498

				42.96		100.255

				42.98		100.255

				43		100.255

				43.02		100.2498

				43.04		100.2498

				43.06		100.2498

				43.08		100.255

				43.09		100.255

				43.11		100.255

				43.13		100.2498

				43.15		100.255

				43.17		100.255

				43.19		100.255

				43.2		100.255

				43.22		100.255

				43.24		100.255

				43.26		100.255

				43.28		100.255

				43.3		100.255

				43.32		100.255

				43.33		100.255

				43.35		100.255

				43.37		100.255

				43.39		100.255

				43.41		100.255

				43.43		100.255

				43.45		100.255

				43.46		100.255

				43.48		100.255

				43.5		100.255

				43.52		100.255

				43.54		100.255

				43.56		100.255

				43.58		100.255

				43.59		100.255

				43.61		100.255

				43.63		100.255

				43.65		100.255

				43.67		100.255

				43.69		100.255

				43.71		100.255

				43.73		100.255

				43.74		100.255

				43.76		100.2602

				43.78		100.255

				43.8		100.255

				43.82		100.255

				43.84		100.255

				43.86		100.255

				43.88		100.255

				43.89		100.255

				43.91		100.255

				43.93		100.255

				43.95		100.2602

				43.97		100.255

				43.99		100.255

				44.01		100.2602

				44.03		100.2602

				44.04		100.2602

				44.06		100.2602

				44.08		100.255

				44.1		100.2602

				44.12		100.2602

				44.14		100.2602

				44.16		100.2602

				44.18		100.2602

				44.19		100.2602

				44.21		100.2602

				44.23		100.2602

				44.25		100.2602

				44.27		100.2602

				44.29		100.2602

				44.31		100.2602

				44.33		100.2602

				44.34		100.2602

				44.36		100.2602

				44.38		100.2602

				44.4		100.2602

				44.42		100.2602

				44.44		100.2602

				44.46		100.2602

				44.48		100.2602

				44.5		100.2602

				44.51		100.2602

				44.53		100.2602

				44.55		100.2602

				44.57		100.2602

				44.59		100.2654

				44.61		100.2602

				44.63		100.2602

				44.65		100.2654

				44.67		100.2654

				44.68		100.2654

				44.7		100.2654

				44.72		100.2654

				44.74		100.2654

				44.76		100.2654

				44.78		100.2654

				44.8		100.2654

				44.82		100.2654

				44.84		100.2654

				44.86		100.2602

				44.87		100.2602

				44.89		100.2654

				44.91		100.2602

				44.93		100.2602

				44.95		100.2654

				44.97		100.2654

				44.99		100.2654

				45.01		100.2654

				45.03		100.2654

				45.05		100.2654

				45.06		100.2654

				45.08		100.2654

				45.1		100.2654

				45.12		100.2654

				45.14		100.2602

				45.16		100.2602

				45.18		100.2602

				45.2		100.2602

				45.22		100.2602

				45.24		100.2602

				45.25		100.2602

				45.27		100.2602

				45.29		100.2654

				45.31		100.2654

				45.33		100.2654

				45.35		100.2602

				45.37		100.2654

				45.39		100.2654

				45.41		100.2654

				45.43		100.2654

				45.45		100.2654

				45.46		100.2654

				45.48		100.2654

				45.5		100.2654

				45.52		100.2654

				45.54		100.2602

				45.56		100.2654

				45.58		100.2654

				45.6		100.2654

				45.62		100.2602

				45.64		100.2602

				45.66		100.2654

				45.67		100.2654

				45.69		100.2654

				45.71		100.2654

				45.73		100.2654

				45.75		100.2654

				45.77		100.2654

				45.79		100.2654

				45.81		100.2654

				45.83		100.2654

				45.85		100.2654

				45.87		100.2654

				45.89		100.2654

				45.9		100.2654

				45.92		100.2654

				45.94		100.2654

				45.96		100.2654

				45.98		100.2654

				46		100.2654

				46.02		100.2654

				46.04		100.2654

				46.06		100.2654

				46.08		100.2654

				46.1		100.2654

				46.12		100.2654

				46.14		100.2654

				46.15		100.2654

				46.17		100.2654

				46.19		100.2654

				46.21		100.2654

				46.23		100.2654

				46.25		100.2654

				46.27		100.2654

				46.29		100.2654

				46.31		100.2654

				46.33		100.2654

				46.35		100.2654

				46.37		100.2654

				46.39		100.2654

				46.4		100.2654

				46.42		100.2654

				46.44		100.2654

				46.46		100.2654

				46.48		100.2654

				46.5		100.2654

				46.52		100.2654

				46.54		100.2654

				46.56		100.2706

				46.58		100.2706

				46.6		100.2706

				46.62		100.2706

				46.64		100.2706

				46.66		100.2706

				46.67		100.2706

				46.69		100.2706

				46.71		100.2706

				46.73		100.2706

				46.75		100.2706

				46.77		100.2706

				46.79		100.2706

				46.81		100.2706

				46.83		100.2706

				46.85		100.2706

				46.87		100.2706

				46.89		100.2706

				46.91		100.2758

				46.93		100.2758

				46.95		100.2758

				46.97		100.2758

				46.98		100.2758

				47		100.2758

				47.02		100.2758

				47.04		100.2758

				47.06		100.2758

				47.08		100.2758

				47.1		100.2758

				47.12		100.2758

				47.14		100.2758

				47.16		100.2758

				47.18		100.2758

				47.2		100.2758

				47.22		100.2758

				47.24		100.2758

				47.26		100.2758

				47.28		100.2758

				47.3		100.2758

				47.31		100.2758

				47.33		100.2758

				47.35		100.2758

				47.37		100.281

				47.39		100.2758

				47.41		100.2758

				47.43		100.2758

				47.45		100.281

				47.47		100.2758

				47.49		100.2758

				47.51		100.281

				47.53		100.2758

				47.55		100.2758

				47.57		100.2758

				47.59		100.2758

				47.61		100.2758

				47.63		100.2758

				47.65		100.2758

				47.67		100.2758

				47.69		100.2758

				47.71		100.2758

				47.72		100.2758

				47.74		100.2758

				47.76		100.2758

				47.78		100.2758

				47.8		100.2758

				47.82		100.2758

				47.84		100.2758

				47.86		100.2758

				47.88		100.2758

				47.9		100.2758

				47.92		100.2758

				47.94		100.2758

				47.96		100.2758

				47.98		100.2758

				48		100.2758

				48.02		100.2758

				48.04		100.2758

				48.06		100.2758

				48.08		100.2758

				48.1		100.2758

				48.12		100.2758

				48.14		100.2758

				48.16		100.2758

				48.17		100.2758

				48.19		100.2758

				48.21		100.2758

				48.23		100.2758

				48.25		100.2758

				48.27		100.2758

				48.29		100.2758

				48.31		100.2758

				48.33		100.2758

				48.35		100.2758

				48.37		100.2758

				48.39		100.2758

				48.41		100.2758

				48.43		100.2758

				48.45		100.2758

				48.47		100.2706

				48.49		100.2706

				48.51		100.2706

				48.53		100.2758

				48.55		100.2706

				48.57		100.2706

				48.59		100.2706

				48.61		100.2706

				48.63		100.2706

				48.65		100.2706

				48.67		100.2758

				48.69		100.2706

				48.71		100.2758

				48.72		100.2706

				48.74		100.2706

				48.76		100.2706

				48.78		100.2758

				48.8		100.2706

				48.82		100.2706

				48.84		100.2706

				48.86		100.2758

				48.88		100.2706

				48.9		100.2706

				48.92		100.2758

				48.94		100.2758

				48.96		100.2758

				48.98		100.2758

				49		100.2758

				49.02		100.2758

				49.04		100.2758

				49.06		100.2758

				49.08		100.2758

				49.1		100.2758

				49.12		100.2758

				49.14		100.2758

				49.16		100.2758

				49.18		100.2758

				49.2		100.2758

				49.22		100.2758

				49.24		100.2758

				49.26		100.2758

				49.28		100.2758

				49.3		100.2758

				49.32		100.2758

				49.34		100.2758

				49.36		100.2758

				49.38		100.2758

				49.4		100.2758

				49.42		100.2758

				49.44		100.2758

				49.46		100.2758

				49.47		100.2758

				49.49		100.2758

				49.51		100.2758

				49.53		100.2758

				49.55		100.2758

				49.57		100.2758

				49.59		100.2758

				49.61		100.2758

				49.63		100.281

				49.65		100.281

				49.67		100.281

				49.69		100.281

				49.71		100.281

				49.73		100.281

				49.75		100.281

				49.77		100.281

				49.79		100.281

				49.81		100.281

				49.83		100.281

				49.85		100.281

				49.87		100.281

				49.89		100.281

				49.91		100.281

				49.93		100.281

				49.95		100.281

				49.97		100.281

				49.99		100.2862

				50.01		100.281

				50.03		100.281

				50.05		100.2862

				50.07		100.2862

				50.09		100.2862

				50.11		100.2862

				50.13		100.281

				50.15		100.281

				50.17		100.281

				50.19		100.281

				50.21		100.281

				50.23		100.281

				50.25		100.281

				50.27		100.281

				50.29		100.281

				50.31		100.281

				50.33		100.281

				50.35		100.281

				50.37		100.281

				50.39		100.2862

				50.41		100.281

				50.43		100.2862

				50.45		100.2862

				50.47		100.2862

				50.49		100.2862

				50.51		100.2862

				50.53		100.2862

				50.55		100.2862

				50.57		100.2862

				50.59		100.2862

				50.61		100.281

				50.63		100.2862

				50.65		100.2862

				50.67		100.281

				50.69		100.281

				50.71		100.281

				50.73		100.281

				50.75		100.281

				50.77		100.281

				50.79		100.281

				50.81		100.281

				50.83		100.281

				50.85		100.281

				50.87		100.281

				50.89		100.281

				50.91		100.281

				50.93		100.281

				50.95		100.281

				50.97		100.281

				50.99		100.281

				51.01		100.281

				51.03		100.281

				51.05		100.281

				51.07		100.281

				51.09		100.281

				51.11		100.281

				51.13		100.281

				51.15		100.281

				51.17		100.281

				51.19		100.281

				51.21		100.281

				51.23		100.281

				51.25		100.281

				51.27		100.281

				51.29		100.281

				51.31		100.281

				51.33		100.281

				51.35		100.2862

				51.37		100.2862

				51.39		100.2862

				51.41		100.2862

				51.43		100.2862

				51.45		100.2862

				51.47		100.2862

				51.49		100.2862

				51.51		100.2862

				51.53		100.2862

				51.55		100.2862

				51.57		100.2862

				51.59		100.2862

				51.61		100.2862

				51.63		100.2862

				51.65		100.2862

				51.67		100.2862

				51.69		100.2862

				51.71		100.2862

				51.73		100.2862

				51.75		100.2862

				51.77		100.2862

				51.79		100.2862

				51.81		100.2862

				51.83		100.2862

				51.85		100.2862

				51.87		100.2862

				51.89		100.2862

				51.91		100.2862

				51.93		100.2862

				51.95		100.2862

				51.97		100.2862

				51.99		100.2862

				52.01		100.2862

				52.03		100.2862

				52.05		100.2862

				52.07		100.2862

				52.09		100.2862

				52.11		100.2862

				52.13		100.2862

				52.15		100.2862

				52.17		100.2862

				52.19		100.2862

				52.21		100.2862

				52.23		100.2862

				52.25		100.2862

				52.27		100.2862

				52.29		100.2862

				52.31		100.2862

				52.33		100.2862

				52.35		100.2862

				52.37		100.2862

				52.39		100.2862

				52.41		100.2862

				52.43		100.2862

				52.45		100.2862

				52.47		100.2862

				52.49		100.2862

				52.51		100.2914

				52.53		100.2862

				52.55		100.2862

				52.58		100.2862

				52.6		100.2862

				52.62		100.2862

				52.64		100.2914

				52.66		100.2914

				52.68		100.2914

				52.7		100.2914

				52.72		100.2914

				52.74		100.2914

				52.76		100.2914

				52.78		100.2914

				52.8		100.2914

				52.82		100.2914

				52.84		100.2914

				52.86		100.2914

				52.88		100.2914

				52.9		100.2914

				52.92		100.2914

				52.94		100.2914

				52.96		100.2914

				52.98		100.2914

				53		100.2914

				53.02		100.2914

				53.04		100.2914

				53.06		100.2914

				53.08		100.2914

				53.1		100.2914

				53.12		100.2914

				53.14		100.2914

				53.16		100.2966

				53.18		100.2914

				53.2		100.2966

				53.22		100.2966

				53.24		100.2966

				53.26		100.2914

				53.28		100.2966

				53.3		100.2914

				53.32		100.2966

				53.34		100.2914

				53.36		100.2966

				53.38		100.2914

				53.4		100.2914

				53.42		100.2914

				53.44		100.2914

				53.46		100.2914

				53.49		100.2914

				53.51		100.2914

				53.53		100.2914

				53.55		100.2914

				53.57		100.2914

				53.59		100.2914

				53.61		100.2914

				53.63		100.2914

				53.65		100.2914

				53.67		100.2914

				53.69		100.2914

				53.71		100.2914

				53.73		100.2914

				53.75		100.2914

				53.77		100.2914

				53.79		100.2914

				53.81		100.2914

				53.83		100.2914

				53.85		100.2914

				53.87		100.2914

				53.89		100.2914

				53.91		100.2914

				53.93		100.2914

				53.95		100.2914

				53.97		100.2914

				53.99		100.2914

				54.01		100.2914

				54.03		100.2914

				54.05		100.2914

				54.07		100.2914

				54.09		100.2966

				54.11		100.2914

				54.13		100.2966

				54.15		100.2914

				54.18		100.2966

				54.2		100.2966

				54.22		100.2966

				54.24		100.2966

				54.26		100.2966

				54.28		100.2966

				54.3		100.2966

				54.32		100.2966

				54.34		100.2966

				54.36		100.2966

				54.38		100.2966

				54.4		100.2966

				54.42		100.2966

				54.44		100.2966

				54.46		100.2966

				54.48		100.2966

				54.5		100.2966

				54.52		100.2966

				54.54		100.2966

				54.56		100.2966

				54.58		100.2966

				54.6		100.2966

				54.62		100.2966

				54.64		100.2966

				54.66		100.2966

				54.68		100.2966

				54.7		100.2966

				54.72		100.2966

				54.75		100.2966

				54.77		100.2966

				54.79		100.2966

				54.81		100.2966

				54.83		100.2966

				54.85		100.2966

				54.87		100.2966

				54.89		100.2966

				54.91		100.2966

				54.93		100.2966

				54.95		100.2966

				54.97		100.2966

				54.99		100.2966

				55.01		100.2966

				55.03		100.2966

				55.05		100.2966

				55.07		100.2966

				55.09		100.2966

				55.11		100.2966

				55.13		100.2966

				55.15		100.2966

				55.17		100.2966

				55.19		100.2966

				55.21		100.2966

				55.23		100.2966

				55.25		100.2966

				55.28		100.2966

				55.3		100.2966

				55.32		100.2966

				55.34		100.2966

				55.36		100.2966

				55.38		100.2966

				55.4		100.3018

				55.42		100.2966

				55.44		100.3018

				55.46		100.3018

				55.48		100.3018

				55.5		100.3018

				55.52		100.3018

				55.54		100.3018

				55.56		100.3018

				55.58		100.3018

				55.6		100.3018

				55.62		100.3018

				55.64		100.3018

				55.66		100.3018

				55.68		100.3018

				55.7		100.3018

				55.72		100.3018

				55.74		100.3018

				55.77		100.3018

				55.79		100.3018

				55.81		100.3018

				55.83		100.3018

				55.85		100.3018

				55.87		100.3018

				55.89		100.3018

				55.91		100.3018

				55.93		100.3018

				55.95		100.3018

				55.97		100.3018

				55.99		100.3018

				56.01		100.3018

				56.03		100.3018

				56.05		100.3018

				56.07		100.3018

				56.09		100.3018

				56.11		100.3018

				56.13		100.3018

				56.15		100.3018

				56.17		100.3018

				56.2		100.3018

				56.22		100.3018

				56.24		100.3018

				56.26		100.3018

				56.28		100.3018

				56.3		100.3018

				56.32		100.2966

				56.34		100.2966

				56.36		100.3018

				56.38		100.3018

				56.4		100.3018

				56.42		100.3018

				56.44		100.3018

				56.46		100.3018

				56.48		100.3018

				56.5		100.3018

				56.52		100.3018

				56.54		100.3018

				56.56		100.3018

				56.58		100.3018

				56.61		100.3018

				56.63		100.3018

				56.65		100.3018

				56.67		100.3018

				56.69		100.3018

				56.71		100.3018

				56.73		100.3018

				56.75		100.3018

				56.77		100.3018

				56.79		100.3018

				56.81		100.3018

				56.83		100.3018

				56.85		100.3018

				56.87		100.3018

				56.89		100.3018

				56.91		100.3018

				56.93		100.307

				56.95		100.307

				56.97		100.307

				57		100.3018

				57.02		100.307

				57.04		100.3018

				57.06		100.3018

				57.08		100.3018

				57.1		100.3018

				57.12		100.3018

				57.14		100.3018

				57.16		100.3018

				57.18		100.3018

				57.2		100.3018

				57.22		100.3018

				57.24		100.3018

				57.26		100.3018

				57.28		100.3018

				57.3		100.3018

				57.32		100.3018

				57.34		100.3018

				57.37		100.3018

				57.39		100.3018

				57.41		100.3018

				57.43		100.3018

				57.45		100.3018

				57.47		100.3018

				57.49		100.3018

				57.51		100.3018

				57.53		100.3018

				57.55		100.3018

				57.57		100.3018

				57.59		100.3018

				57.61		100.3018

				57.63		100.3018

				57.65		100.3018

				57.67		100.3018

				57.69		100.3018

				57.71		100.3018

				57.74		100.3018

				57.76		100.3018

				57.78		100.3018

				57.8		100.3018

				57.82		100.3018

				57.84		100.3018

				57.86		100.3018

				57.88		100.3018

				57.9		100.3018

				57.92		100.3018

				57.94		100.3018

				57.96		100.3018

				57.98		100.3018

				58		100.3018

				58.02		100.3018

				58.04		100.3018

				58.06		100.3018

				58.08		100.3018

				58.11		100.3018

				58.13		100.3018

				58.15		100.3018

				58.17		100.3018

				58.19		100.3018

				58.21		100.3018

				58.23		100.3018

				58.25		100.3018

				58.27		100.3018

				58.29		100.3018

				58.31		100.307

				58.33		100.307

				58.35		100.307

				58.37		100.307

				58.39		100.3018

				58.41		100.307

				58.44		100.307

				58.46		100.307

				58.48		100.307

				58.5		100.307

				58.52		100.307

				58.54		100.307

				58.56		100.307

				58.58		100.307

				58.6		100.307

				58.62		100.307

				58.64		100.307

				58.66		100.307

				58.68		100.307

				58.7		100.307

				58.72		100.307

				58.74		100.307

				58.77		100.307

				58.79		100.307

				58.81		100.307

				58.83		100.307

				58.85		100.307

				58.87		100.307

				58.89		100.307

				58.91		100.307

				58.93		100.307

				58.95		100.307

				58.97		100.307

				58.99		100.307

				59.01		100.307

				59.03		100.307

				59.05		100.307

				59.07		100.307

				59.1		100.307

				59.12		100.307

				59.14		100.307

				59.16		100.307

				59.18		100.307

				59.2		100.307

				59.22		100.307

				59.24		100.3122

				59.26		100.3122

				59.28		100.3122

				59.3		100.3122

				59.32		100.3122

				59.34		100.3122

				59.36		100.3122

				59.38		100.3122

				59.4		100.3122

				59.43		100.3122

				59.45		100.3122

				59.47		100.3122

				59.49		100.3122

				59.51		100.3122

				59.53		100.3122

				59.55		100.3122

				59.57		100.3174

				59.59		100.3174

				59.61		100.3174

				59.63		100.3174

				59.65		100.3174

				59.67		100.3174

				59.69		100.3174

				59.71		100.3174

				59.74		100.3174

				59.76		100.3174

				59.78		100.3174

				59.8		100.3174

				59.82		100.3174

				59.84		100.3226

				59.86		100.3226

				59.88		100.3226

				59.9		100.3226

				59.92		100.3226

				59.94		100.3226

				59.96		100.3226

				59.98		100.3226

				60		100.3226

				60.02		100.3226

				60.04		100.3226

				60.07		100.3226

				60.09		100.3226

				60.11		100.3226

				60.13		100.3226

				60.15		100.3226

				60.17		100.3278

				60.19		100.3278

				60.21		100.3278

				60.23		100.3278

				60.25		100.3278

				60.27		100.3278

				60.29		100.3278

				60.31		100.3278

				60.33		100.3278

				60.35		100.3278

				60.38		100.3278

				60.4		100.3278

				60.42		100.333

				60.44		100.333

				60.46		100.333

				60.48		100.333

				60.5		100.333

				60.52		100.333

				60.54		100.333

				60.56		100.333

				60.58		100.333

				60.6		100.333

				60.62		100.333

				60.64		100.333

				60.66		100.333

				60.68		100.333

				60.71		100.333

				60.73		100.333

				60.75		100.333

				60.77		100.333

				60.79		100.3382

				60.81		100.333

				60.83		100.3382

				60.85		100.3382

				60.87		100.3382

				60.89		100.3382

				60.91		100.3382

				60.93		100.3382

				60.95		100.3382

				60.97		100.3382

				60.99		100.3382

				61.01		100.3382

				61.03		100.3382

				61.06		100.3382

				61.08		100.3382

				61.1		100.3382

				61.12		100.3382

				61.14		100.3382

				61.16		100.3382

				61.18		100.3382

				61.2		100.3382

				61.22		100.3382

				61.24		100.3434

				61.26		100.3434

				61.28		100.3382

				61.3		100.3382

				61.32		100.3434

				61.34		100.3382

				61.36		100.3382

				61.38		100.3382

				61.41		100.3382

				61.43		100.3382

				61.45		100.3382

				61.47		100.3382

				61.49		100.3382

				61.51		100.3382

				61.53		100.3382

				61.55		100.3382

				61.57		100.3382

				61.59		100.3382

				61.61		100.3382

				61.63		100.3382

				61.65		100.3382

				61.67		100.3382

				61.69		100.3382

				61.71		100.3382

				61.74		100.3382

				61.76		100.3382

				61.78		100.3382

				61.8		100.3382

				61.82		100.3382

				61.84		100.3382

				61.86		100.3382

				61.88		100.3382

				61.9		100.3382

				61.92		100.3382

				61.94		100.3382

				61.96		100.3382

				61.98		100.3382

				62		100.3382

				62.02		100.3382

				62.04		100.3382

				62.06		100.3382

				62.09		100.3382

				62.11		100.3382

				62.13		100.3382

				62.15		100.3382

				62.17		100.3382

				62.19		100.3382

				62.21		100.3382

				62.23		100.3382

				62.25		100.3382

				62.27		100.3382

				62.29		100.3382

				62.31		100.3382

				62.33		100.3382

				62.35		100.3382

				62.37		100.3382

				62.39		100.3382

				62.42		100.3382

				62.44		100.3434

				62.46		100.3382

				62.48		100.3382

				62.5		100.3382

				62.52		100.3382

				62.54		100.3382

				62.56		100.3382

				62.58		100.3382

				62.6		100.3382

				62.62		100.3382

				62.64		100.3382

				62.66		100.3382

				62.68		100.3382

				62.7		100.3434

				62.72		100.3382

				62.74		100.3382

				62.77		100.3434

				62.79		100.3434

				62.81		100.3434

				62.83		100.3434

				62.85		100.3434

				62.87		100.3434

				62.89		100.3434

				62.91		100.3382

				62.93		100.3434

				62.95		100.3382

				62.97		100.3434

				62.99		100.3382

				63.01		100.3382

				63.03		100.3382

				63.05		100.3434

				63.07		100.3382

				63.09		100.3434

				63.12		100.3434

				63.14		100.3434

				63.16		100.3434

				63.18		100.3434

				63.2		100.3434

				63.22		100.3434

				63.24		100.3434

				63.26		100.3434

				63.28		100.3434

				63.3		100.3434

				63.32		100.3434

				63.34		100.3434

				63.36		100.3434

				63.38		100.3434

				63.4		100.3434

				63.42		100.3382

				63.44		100.3434

				63.46		100.3434

				63.49		100.3434

				63.51		100.3434

				63.53		100.3434

				63.55		100.3434

				63.57		100.3434

				63.59		100.3434

				63.61		100.3434

				63.63		100.3434

				63.65		100.3434

				63.67		100.3434

				63.69		100.3434

				63.71		100.3434

				63.73		100.3434

				63.75		100.3434

				63.77		100.3434

				63.79		100.3434

				63.81		100.3434

				63.84		100.3434

				63.86		100.3434

				63.88		100.3434

				63.9		100.3434

				63.92		100.3434

				63.94		100.3434

				63.96		100.3434

				63.98		100.3434

				64		100.3434

				64.02		100.3434

				64.04		100.3434

				64.06		100.3434

				64.08		100.3434

				64.1		100.3434

				64.12		100.3434

				64.14		100.3434

				64.16		100.3434

				64.19		100.3434

				64.21		100.3434

				64.23		100.3434

				64.25		100.3434

				64.27		100.3434

				64.29		100.3434

				64.31		100.3434

				64.33		100.3434

				64.35		100.3434

				64.37		100.3434

				64.39		100.3434

				64.41		100.3434

				64.43		100.3434

				64.45		100.3434

				64.47		100.3382

				64.49		100.3434

				64.52		100.3382

				64.54		100.3434

				64.56		100.3434

				64.58		100.3434

				64.6		100.3382

				64.62		100.3434

				64.64		100.3434

				64.66		100.3382

				64.68		100.3434

				64.7		100.3382

				64.72		100.3382

				64.74		100.3382

				64.76		100.3382

				64.78		100.3382

				64.8		100.3382

				64.82		100.3382

				64.85		100.3382

				64.87		100.3382

				64.89		100.3382

				64.91		100.3382

				64.93		100.3382

				64.95		100.3382

				64.97		100.3382

				64.99		100.3382

				65.01		100.3382

				65.03		100.3382

				65.05		100.3382

				65.07		100.3382

				65.09		100.3382

				65.11		100.3382

				65.13		100.3382

				65.15		100.3382

				65.18		100.3382

				65.2		100.3382

				65.22		100.3382

				65.24		100.3382

				65.26		100.3382

				65.28		100.3382

				65.3		100.3382

				65.32		100.3382

				65.34		100.3382

				65.36		100.3382

				65.38		100.3382

				65.4		100.3382

				65.42		100.3382

				65.44		100.3382

				65.46		100.3382

				65.48		100.3382

				65.51		100.3382

				65.53		100.3382

				65.55		100.3382

				65.57		100.3382

				65.59		100.3382

				65.61		100.3382

				65.63		100.3382

				65.65		100.3382

				65.67		100.3382

				65.69		100.3382

				65.71		100.3382

				65.73		100.3382

				65.75		100.3382

				65.77		100.3382

				65.79		100.3382

				65.82		100.3382

				65.84		100.3382

				65.86		100.3382

				65.88		100.3382

				65.9		100.3382

				65.92		100.3434

				65.94		100.3434

				65.96		100.3434

				65.98		100.3434

				66		100.3434

				66.02		100.3434

				66.04		100.3434

				66.06		100.3434

				66.08		100.3434

				66.1		100.3434

				66.13		100.3434

				66.15		100.3434

				66.17		100.3434

				66.19		100.3434

				66.21		100.3434

				66.23		100.3434

				66.25		100.3434

				66.27		100.3434

				66.29		100.3434

				66.31		100.3434

				66.33		100.3434

				66.35		100.3434

				66.37		100.3434

				66.39		100.3434

				66.41		100.3434

				66.44		100.3434

				66.46		100.3434

				66.48		100.3434

				66.5		100.3486

				66.52		100.3486

				66.54		100.3486

				66.56		100.3486

				66.58		100.3486

				66.6		100.3486

				66.62		100.3486

				66.64		100.3486

				66.66		100.3486

				66.68		100.3486

				66.7		100.3486

				66.72		100.3486

				66.75		100.3486

				66.77		100.3539

				66.79		100.3539

				66.81		100.3539

				66.83		100.3539

				66.85		100.3539

				66.87		100.3539

				66.89		100.3539

				66.91		100.3539

				66.93		100.3539

				66.95		100.3539

				66.97		100.3591

				66.99		100.3591

				67.01		100.3591

				67.04		100.3591

				67.06		100.3591

				67.08		100.3591

				67.1		100.3591

				67.12		100.3591

				67.14		100.3539

				67.16		100.3591

				67.18		100.3591

				67.2		100.3591

				67.22		100.3539

				67.24		100.3539

				67.26		100.3539

				67.28		100.3539

				67.3		100.3591

				67.33		100.3539

				67.35		100.3591

				67.37		100.3539

				67.39		100.3591

				67.41		100.3591

				67.43		100.3591

				67.45		100.3591

				67.47		100.3591

				67.49		100.3591

				67.51		100.3591

				67.53		100.3591

				67.55		100.3591

				67.57		100.3591

				67.6		100.3591

				67.62		100.3591

				67.64		100.3591

				67.66		100.3591

				67.68		100.3591

				67.7		100.3591

				67.72		100.3591

				67.74		100.3591

				67.76		100.3591

				67.78		100.3591

				67.8		100.3591

				67.82		100.3591

				67.84		100.3591

				67.87		100.3591

				67.89		100.3591

				67.91		100.3591

				67.93		100.3591

				67.95		100.3591

				67.97		100.3591

				67.99		100.3591

				68.01		100.3591

				68.03		100.3591

				68.05		100.3591

				68.07		100.3591

				68.09		100.3591

				68.11		100.3591

				68.14		100.3591

				68.16		100.3591

				68.18		100.3591

				68.2		100.3591

				68.22		100.3591

				68.24		100.3591

				68.26		100.3591

				68.28		100.3591

				68.3		100.3591

				68.32		100.3591

				68.34		100.3591

				68.36		100.3591

				68.38		100.3591

				68.41		100.3591

				68.43		100.3591

				68.45		100.3591

				68.47		100.3591

				68.49		100.3591

				68.51		100.3591

				68.53		100.3591

				68.55		100.3539

				68.57		100.3591

				68.59		100.3539

				68.61		100.3539

				68.63		100.3539

				68.66		100.3539

				68.68		100.3539

				68.7		100.3539

				68.72		100.3539

				68.74		100.3539

				68.76		100.3539

				68.78		100.3539

				68.8		100.3539

				68.82		100.3539

				68.84		100.3539

				68.86		100.3539

				68.88		100.3539

				68.91		100.3539

				68.93		100.3539

				68.95		100.3539

				68.97		100.3486

				68.99		100.3539

				69.01		100.3539

				69.03		100.3486

				69.05		100.3486

				69.07		100.3539

				69.09		100.3539

				69.11		100.3539

				69.13		100.3539

				69.16		100.3539

				69.18		100.3539

				69.2		100.3539

				69.22		100.3539

				69.24		100.3539

				69.26		100.3539

				69.28		100.3539

				69.3		100.3539

				69.32		100.3539

				69.34		100.3539

				69.36		100.3539

				69.39		100.3539

				69.41		100.3539

				69.43		100.3539

				69.45		100.3539

				69.47		100.3539

				69.49		100.3539

				69.51		100.3539

				69.53		100.3539

				69.55		100.3539

				69.57		100.3539

				69.59		100.3539

				69.61		100.3539

				69.64		100.3539

				69.66		100.3539

				69.68		100.3539

				69.7		100.3539

				69.72		100.3539

				69.74		100.3539

				69.76		100.3539

				69.78		100.3539

				69.8		100.3539

				69.82		100.3539

				69.84		100.3539

				69.87		100.3539

				69.89		100.3539

				69.91		100.3539

				69.93		100.3539

				69.95		100.3539

				69.97		100.3539

				69.99		100.3539

				70.01		100.3539

				70.03		100.3539

				70.05		100.3539

				70.07		100.3539

				70.1		100.3539

				70.12		100.3539

				70.14		100.3539

				70.16		100.3539

				70.18		100.3539

				70.2		100.3539

				70.22		100.3539

				70.24		100.3539

				70.26		100.3539

				70.28		100.3539

				70.3		100.3539

				70.33		100.3539

				70.35		100.3539

				70.37		100.3539

				70.39		100.3591

				70.41		100.3539

				70.43		100.3539

				70.45		100.3591

				70.47		100.3539

				70.49		100.3539

				70.51		100.3539

				70.53		100.3539

				70.56		100.3539

				70.58		100.3539

				70.6		100.3539

				70.62		100.3539

				70.64		100.3539

				70.66		100.3539

				70.68		100.3539

				70.7		100.3539

				70.72		100.3539

				70.74		100.3591

				70.76		100.3591

				70.79		100.3591

				70.81		100.3591

				70.83		100.3591

				70.85		100.3539

				70.87		100.3591

				70.89		100.3591

				70.91		100.3591

				70.93		100.3591

				70.95		100.3591

				70.97		100.3591

				70.99		100.3591

				71.02		100.3591

				71.04		100.3591

				71.06		100.3591

				71.08		100.3591

				71.1		100.3591

				71.12		100.3591

				71.14		100.3591

				71.16		100.3591

				71.18		100.3591

				71.2		100.3591

				71.22		100.3591

				71.25		100.3591

				71.27		100.3591

				71.29		100.3591

				71.31		100.3591

				71.33		100.3591

				71.35		100.3591

				71.37		100.3591

				71.39		100.3591

				71.41		100.3591

				71.43		100.3591

				71.46		100.3591

				71.48		100.3591

				71.5		100.3591

				71.52		100.3591

				71.54		100.3591

				71.56		100.3591

				71.58		100.3591

				71.6		100.3591

				71.62		100.3591

				71.64		100.3591

				71.66		100.3591

				71.69		100.3591

				71.71		100.3591

				71.73		100.3591

				71.75		100.3591

				71.77		100.3591

				71.79		100.3591

				71.81		100.3591

				71.83		100.3591

				71.85		100.3591

				71.87		100.3591

				71.9		100.3591

				71.92		100.3591

				71.94		100.3591

				71.96		100.3591

				71.98		100.3591

				72		100.3591

				72.02		100.3591

				72.04		100.3591

				72.06		100.3591

				72.08		100.3591

				72.1		100.3591

				72.13		100.3591

				72.15		100.3591

				72.17		100.3591

				72.19		100.3591

				72.21		100.3591

				72.23		100.3591

				72.25		100.3591

				72.27		100.3591

				72.29		100.3591

				72.31		100.3591

				72.34		100.3591

				72.36		100.3591

				72.38		100.3591

				72.4		100.3591

				72.42		100.3591

				72.44		100.3591

				72.46		100.3591

				72.48		100.3591

				72.5		100.3591

				72.52		100.3591

				72.55		100.3591

				72.57		100.3591

				72.59		100.3591

				72.61		100.3591

				72.63		100.3591

				72.65		100.3591

				72.67		100.3643

				72.69		100.3643

				72.71		100.3591

				72.73		100.3643

				72.76		100.3643

				72.78		100.3643

				72.8		100.3643

				72.82		100.3643

				72.84		100.3643

				72.86		100.3643

				72.88		100.3643

				72.9		100.3643

				72.92		100.3643

				72.94		100.3643

				72.97		100.3643

				72.99		100.3643

				73.01		100.3643

				73.03		100.3643

				73.05		100.3643

				73.07		100.3643

				73.09		100.3643

				73.11		100.3643

				73.13		100.3643

				73.15		100.3643

				73.17		100.3643

				73.2		100.3591

				73.22		100.3643

				73.24		100.3591

				73.26		100.3591

				73.28		100.3591

				73.3		100.3591

				73.32		100.3643

				73.34		100.3643

				73.36		100.3643

				73.38		100.3643

				73.41		100.3643

				73.43		100.3643

				73.45		100.3643

				73.47		100.3643

				73.49		100.3591

				73.51		100.3643

				73.53		100.3643

				73.55		100.3643

				73.57		100.3643

				73.59		100.3643

				73.62		100.3643

				73.64		100.3643

				73.66		100.3643

				73.68		100.3643

				73.7		100.3643

				73.72		100.3643

				73.74		100.3643

				73.76		100.3643

				73.78		100.3643

				73.8		100.3643

				73.83		100.3643

				73.85		100.3643

				73.87		100.3643

				73.89		100.3643

				73.91		100.3643

				73.93		100.3643

				73.95		100.3643

				73.97		100.3643

				73.99		100.3643

				74.01		100.3643

				74.04		100.3643

				74.06		100.3643

				74.08		100.3643

				74.1		100.3643

				74.12		100.3643

				74.14		100.3643

				74.16		100.3643

				74.18		100.3643

				74.2		100.3643

				74.22		100.3643

				74.25		100.3643

				74.27		100.3643

				74.29		100.3643

				74.31		100.3643

				74.33		100.3643

				74.35		100.3643

				74.37		100.3643

				74.39		100.3643

				74.41		100.3643

				74.44		100.3643

				74.46		100.3643

				74.48		100.3643

				74.5		100.3643

				74.52		100.3643

				74.54		100.3643

				74.56		100.3643

				74.58		100.3643

				74.6		100.3643

				74.62		100.3643

				74.65		100.3643

				74.67		100.3643

				74.69		100.3643

				74.71		100.3643

				74.73		100.3643

				74.75		100.3643

				74.77		100.3643

				74.79		100.3643

				74.81		100.3643

				74.83		100.3643

				74.86		100.3643

				74.88		100.3643

				74.9		100.3643

				74.92		100.3643

				74.94		100.3643

				74.96		100.3643

				74.98		100.3591

				75		100.3643

				75.02		100.3643

				75.05		100.3643

				75.07		100.3643

				75.09		100.3643

				75.11		100.3643

				75.13		100.3643

				75.15		100.3643

				75.17		100.3643

				75.19		100.3643

				75.21		100.3643

				75.23		100.3643

				75.26		100.3643

				75.28		100.3643

				75.3		100.3643

				75.32		100.3643

				75.34		100.3643

				75.36		100.3643

				75.38		100.3643

				75.4		100.3643

				75.42		100.3643

				75.44		100.3643

				75.47		100.3643

				75.49		100.3643

				75.51		100.3643

				75.53		100.3643

				75.55		100.3643

				75.57		100.3695

				75.59		100.3695

				75.61		100.3695

				75.63		100.3695

				75.66		100.3695

				75.68		100.3695

				75.7		100.3695

				75.72		100.3643

				75.74		100.3643

				75.76		100.3643

				75.78		100.3643

				75.8		100.3643

				75.82		100.3643

				75.84		100.3643

				75.87		100.3643

				75.89		100.3643

				75.91		100.3643

				75.93		100.3643

				75.95		100.3643

				75.97		100.3695

				75.99		100.3695

				76.01		100.3695

				76.03		100.3695

				76.05		100.3695

				76.08		100.3695

				76.1		100.3695

				76.12		100.3695

				76.14		100.3695

				76.16		100.3695

				76.18		100.3695

				76.2		100.3695

				76.22		100.3695

				76.24		100.3695

				76.27		100.3695

				76.29		100.3695

				76.31		100.3695

				76.33		100.3643

				76.35		100.3695

				76.37		100.3695

				76.39		100.3643

				76.41		100.3643

				76.43		100.3643

				76.46		100.3643

				76.48		100.3695

				76.5		100.3643

				76.52		100.3643

				76.54		100.3695

				76.56		100.3695

				76.58		100.3695

				76.6		100.3643

				76.62		100.3643

				76.64		100.3591

				76.67		100.3539

				76.69		100.3539

				76.71		100.3539

				76.73		100.3539

				76.75		100.3539

				76.77		100.3539

				76.79		100.3539

				76.81		100.3539

				76.83		100.3539

				76.86		100.3539

				76.88		100.3486

				76.9		100.3486

				76.92		100.3486

				76.94		100.3486

				76.96		100.3486

				76.98		100.3486

				77		100.3486

				77.02		100.3486

				77.05		100.3486

				77.07		100.3486

				77.09		100.3434

				77.11		100.3434

				77.13		100.3434

				77.15		100.3434

				77.17		100.3434

				77.19		100.3434

				77.21		100.3434

				77.23		100.3434

				77.26		100.3434

				77.28		100.3382

				77.3		100.3382

				77.32		100.3434

				77.34		100.3434

				77.36		100.3434

				77.38		100.3434

				77.4		100.3434

				77.42		100.3434

				77.45		100.3434

				77.47		100.3434

				77.49		100.3434

				77.51		100.3434

				77.53		100.3434

				77.55		100.3486

				77.57		100.3486

				77.59		100.3486

				77.61		100.3539

				77.64		100.3539

				77.66		100.3591

				77.68		100.3643

				77.7		100.3643

				77.72		100.3643

				77.74		100.3643

				77.76		100.3643

				77.78		100.3643

				77.8		100.3643

				77.83		100.3643

				77.85		100.3643

				77.87		100.3591

				77.89		100.3591

				77.91		100.3591

				77.93		100.3591

				77.95		100.3591

				77.97		100.3591

				77.99		100.3591

				78.01		100.3591

				78.04		100.3591

				78.06		100.3591

				78.08		100.3591

				78.1		100.3591

				78.12		100.3591

				78.14		100.3591

				78.16		100.3591

				78.18		100.3695

				78.2		100.3799

				78.23		100.3903

				78.25		100.3955

				78.27		100.3955

				78.29		100.4007

				78.31		100.4059

				78.33		100.4111

				78.35		100.4111

				78.37		100.4215

				78.39		100.4215

				78.41		100.4215

				78.44		100.4163

				78.46		100.4163

				78.48		100.4215

				78.5		100.4215

				78.52		100.4215

				78.54		100.4163

				78.56		100.4163

				78.58		100.4163

				78.6		100.4111

				78.63		100.4111

				78.65		100.4111

				78.67		100.4111

				78.69		100.4111

				78.71		100.4111

				78.73		100.4059

				78.75		100.4059

				78.77		100.4059

				78.79		100.4007

				78.82		100.4007

				78.84		100.4007

				78.86		100.4007

				78.88		100.3955

				78.9		100.4007

				78.92		100.3955

				78.94		100.3955

				78.96		100.3955

				78.98		100.3955

				79.01		100.3955

				79.03		100.3955

				79.05		100.3955

				79.07		100.3955

				79.09		100.3955

				79.11		100.3955

				79.13		100.3955

				79.15		100.3955

				79.17		100.3955

				79.2		100.3955

				79.22		100.3955

				79.24		100.3955

				79.26		100.3955

				79.28		100.3955

				79.3		100.4007

				79.32		100.3955

				79.34		100.4007

				79.36		100.3955

				79.39		100.3955

				79.41		100.3955

				79.43		100.3955

				79.45		100.3955

				79.47		100.3955

				79.49		100.3955

				79.51		100.3955

				79.53		100.3903

				79.55		100.3903

				79.58		100.3903

				79.6		100.3903

				79.62		100.3903

				79.64		100.3903

				79.66		100.3903

				79.68		100.3903

				79.7		100.3903

				79.72		100.3851

				79.74		100.3851

				79.77		100.3851

				79.79		100.3799

				79.81		100.3799

				79.83		100.3799

				79.85		100.3799

				79.87		100.3799

				79.89		100.3799

				79.91		100.3799

				79.93		100.3799

				79.96		100.3799

				79.98		100.3799

				80		100.3799

				80.02		100.3799

				80.04		100.3799

				80.06		100.3799

				80.08		100.3747

				80.1		100.3799

				80.12		100.3799

				80.15		100.3799

				80.17		100.3799

				80.19		100.3799

				80.21		100.3799

				80.23		100.3799

				80.25		100.3799

				80.27		100.3799

				80.29		100.3799

				80.31		100.3799

				80.34		100.3799

				80.36		100.3799

				80.38		100.3747

				80.4		100.3799

				80.42		100.3799

				80.44		100.3799

				80.46		100.3799

				80.48		100.3799

				80.5		100.3799

				80.53		100.3799

				80.55		100.3799

				80.57		100.3799

				80.59		100.3799

				80.61		100.3799

				80.63		100.3799

				80.65		100.3799

				80.67		100.3799

				80.69		100.3799

				80.72		100.3799

				80.74		100.3799

				80.76		100.3799

				80.78		100.3799

				80.8		100.3799

				80.82		100.3799

				80.84		100.3799

				80.86		100.3799

				80.88		100.3799

				80.91		100.3799

				80.93		100.3799

				80.95		100.3799

				80.97		100.3799

				80.99		100.3799

				81.01		100.3799

				81.03		100.3799

				81.05		100.3799

				81.07		100.3799

				81.1		100.3799

				81.12		100.3799

				81.14		100.3799

				81.16		100.3799

				81.18		100.3799

				81.2		100.3799

				81.22		100.3799

				81.24		100.3799

				81.26		100.3747

				81.29		100.3747

				81.31		100.3747

				81.33		100.3747

				81.35		100.3747

				81.37		100.3747

				81.39		100.3747

				81.41		100.3747

				81.43		100.3747

				81.45		100.3799

				81.48		100.3799

				81.5		100.3799

				81.52		100.3799

				81.54		100.3799

				81.56		100.3799

				81.58		100.3799

				81.6		100.3799

				81.62		100.3799

				81.64		100.3799

				81.67		100.3799

				81.69		100.3799

				81.71		100.3747

				81.73		100.3747

				81.75		100.3747

				81.77		100.3747

				81.79		100.3747

				81.81		100.3747

				81.83		100.3747

				81.86		100.3747

				81.88		100.3747

				81.9		100.3747

				81.92		100.3747

				81.94		100.3747

				81.96		100.3747

				81.98		100.3747

				82		100.3747

				82.02		100.3747

				82.05		100.3747

				82.07		100.3747

				82.09		100.3747

				82.11		100.3747

				82.13		100.3747

				82.15		100.3747

				82.17		100.3747

				82.19		100.3747

				82.21		100.3747

				82.24		100.3747

				82.26		100.3747

				82.28		100.3747

				82.3		100.3747

				82.32		100.3747

				82.34		100.3747

				82.36		100.3747

				82.38		100.3747

				82.4		100.3747

				82.43		100.3747

				82.45		100.3747

				82.47		100.3695

				82.49		100.3695

				82.51		100.3695

				82.53		100.3695

				82.55		100.3695

				82.57		100.3695

				82.59		100.3747

				82.62		100.3695

				82.64		100.3695

				82.66		100.3695

				82.68		100.3695

				82.7		100.3695

				82.72		100.3695

				82.74		100.3695

				82.76		100.3695

				82.78		100.3695

				82.81		100.3695

				82.83		100.3695

				82.85		100.3695

				82.87		100.3695

				82.89		100.3695

				82.91		100.3695

				82.93		100.3695

				82.95		100.3695

				82.97		100.3695

				83		100.3747

				83.02		100.3747

				83.04		100.3747

				83.06		100.3747

				83.08		100.3747

				83.1		100.3747

				83.12		100.3747

				83.14		100.3747

				83.16		100.3747

				83.19		100.3747

				83.21		100.3747

				83.23		100.3747

				83.25		100.3695

				83.27		100.3695

				83.29		100.3695

				83.31		100.3695

				83.33		100.3695

				83.35		100.3695

				83.38		100.3695

				83.4		100.3695

				83.42		100.3695

				83.44		100.3695

				83.46		100.3695

				83.48		100.3695

				83.5		100.3695

				83.52		100.3695

				83.54		100.3695

				83.57		100.3695

				83.59		100.3695

				83.61		100.3643

				83.63		100.3643

				83.65		100.3643

				83.67		100.3643

				83.69		100.3643

				83.71		100.3643

				83.73		100.3591

				83.76		100.3591

				83.78		100.3591

				83.8		100.3591

				83.82		100.3591

				83.84		100.3591

				83.86		100.3591

				83.88		100.3591

				83.9		100.3591

				83.92		100.3539

				83.95		100.3539

				83.97		100.3539

				83.99		100.3539

				84.01		100.3539

				84.03		100.3591

				84.05		100.3591

				84.07		100.3591

				84.09		100.3591

				84.11		100.3591

				84.14		100.3591

				84.16		100.3591

				84.18		100.3591

				84.2		100.3591

				84.22		100.3643

				84.24		100.3643

				84.26		100.3643

				84.28		100.3695

				84.3		100.3695

				84.33		100.3747

				84.35		100.3747

				84.37		100.3747

				84.39		100.3747

				84.41		100.3747

				84.43		100.3747

				84.45		100.3747

				84.47		100.3747

				84.49		100.3747

				84.52		100.3747

				84.54		100.3747

				84.56		100.3747

				84.58		100.3747

				84.6		100.3747

				84.62		100.3747

				84.64		100.3747

				84.66		100.3799

				84.68		100.3747

				84.71		100.3747

				84.73		100.3747

				84.75		100.3747

				84.77		100.3747

				84.79		100.3799

				84.81		100.3747

				84.83		100.3799

				84.85		100.3799

				84.87		100.3799

				84.9		100.3799

				84.92		100.3747

				84.94		100.3747

				84.96		100.3747

				84.98		100.3799

				85		100.3799

				85.02		100.3799

				85.04		100.3799

				85.06		100.3799

				85.09		100.3799

				85.11		100.3799

				85.13		100.3799

				85.15		100.3851

				85.17		100.3851

				85.19		100.3851

				85.21		100.3799

				85.23		100.3799

				85.25		100.3799

				85.28		100.3799

				85.3		100.3799

				85.32		100.3799

				85.34		100.3799

				85.36		100.3799

				85.38		100.3799

				85.4		100.3799

				85.42		100.3799

				85.44		100.3799

				85.47		100.3799

				85.49		100.3799

				85.51		100.3851

				85.53		100.3799

				85.55		100.3799

				85.57		100.3799

				85.59		100.3799

				85.61		100.3799

				85.63		100.3799

				85.66		100.3799

				85.68		100.3799

				85.7		100.3799

				85.72		100.3799

				85.74		100.3799

				85.76		100.3851

				85.78		100.3851

				85.8		100.3851

				85.82		100.3851

				85.85		100.3851

				85.87		100.3851

				85.89		100.3851

				85.91		100.3851

				85.93		100.3903

				85.95		100.3903

				85.97		100.3851

				85.99		100.3903

				86.01		100.3903

				86.04		100.3903

				86.06		100.3851

				86.08		100.3851

				86.1		100.3851

				86.12		100.3851

				86.14		100.3903

				86.16		100.3851

				86.18		100.3903

				86.2		100.3903

				86.23		100.3851

				86.25		100.3851

				86.27		100.3851

				86.29		100.3799

				86.31		100.3799

				86.33		100.3799

				86.35		100.3799

				86.37		100.3747

				86.39		100.3747

				86.42		100.3695

				86.44		100.3695

				86.46		100.3695

				86.48		100.3695

				86.5		100.3695

				86.52		100.3695

				86.54		100.3695

				86.56		100.3695

				86.58		100.3695

				86.61		100.3643

				86.63		100.3695

				86.65		100.3643

				86.67		100.3643

				86.69		100.3643

				86.71		100.3643

				86.73		100.3643

				86.75		100.3643

				86.77		100.3643

				86.8		100.3643

				86.82		100.3643

				86.84		100.3643

				86.86		100.3643

				86.88		100.3643

				86.9		100.3643

				86.92		100.3643

				86.94		100.3643

				86.96		100.3643

				86.99		100.3643

				87.01		100.3643

				87.03		100.3643

				87.05		100.3643

				87.07		100.3643

				87.09		100.3643

				87.11		100.3643

				87.13		100.3643

				87.15		100.3643

				87.18		100.3643

				87.2		100.3643

				87.22		100.3643

				87.24		100.3643

				87.26		100.3643

				87.28		100.3643

				87.3		100.3643

				87.32		100.3643

				87.34		100.3643

				87.37		100.3643

				87.39		100.3643

				87.41		100.3643

				87.43		100.3643

				87.45		100.3643

				87.47		100.3643

				87.49		100.3643

				87.51		100.3643

				87.53		100.3643

				87.56		100.3643

				87.58		100.3643

				87.6		100.3643

				87.62		100.3643

				87.64		100.3643

				87.66		100.3643

				87.68		100.3643

				87.7		100.3643

				87.72		100.3643

				87.75		100.3643

				87.77		100.3643

				87.79		100.3643

				87.81		100.3643

				87.83		100.3643

				87.85		100.3643

				87.87		100.3643

				87.89		100.3643

				87.91		100.3643

				87.94		100.3643

				87.96		100.3643

				87.98		100.3643

				88		100.3643

				88.02		100.3643

				88.04		100.3643

				88.06		100.3643

				88.08		100.3643

				88.1		100.3643

				88.13		100.3643

				88.15		100.3695

				88.17		100.3643

				88.19		100.3591

				88.21		100.3591

				88.23		100.3643

				88.25		100.3643

				88.27		100.3643

				88.29		100.3643

				88.32		100.3643

				88.34		100.3643

				88.36		100.3643

				88.38		100.3643

				88.4		100.3643

				88.42		100.3643

				88.44		100.3643

				88.46		100.3643

				88.48		100.3643

				88.51		100.3643

				88.53		100.3643

				88.55		100.3643

				88.57		100.3643

				88.59		100.3643

				88.61		100.3643

				88.63		100.3643

				88.65		100.3643

				88.67		100.3643

				88.7		100.3643

				88.72		100.3643

				88.74		100.3695

				88.76		100.3643

				88.78		100.3695

				88.8		100.3695

				88.82		100.3695

				88.84		100.3695

				88.86		100.3695

				88.89		100.3695

				88.91		100.3695

				88.93		100.3695

				88.95		100.3695

				88.97		100.3695

				88.99		100.3695

				89.01		100.3695

				89.03		100.3695

				89.05		100.3695

				89.08		100.3695

				89.1		100.3695

				89.12		100.3695

				89.14		100.3695

				89.16		100.3695

				89.18		100.3695

				89.2		100.3695

				89.22		100.3695

				89.24		100.3695

				89.27		100.3747

				89.29		100.3747

				89.31		100.3747

				89.33		100.3747

				89.35		100.3747

				89.37		100.3747

				89.39		100.3747

				89.41		100.3747

				89.43		100.3747

				89.46		100.3695

				89.48		100.3747

				89.5		100.3747

				89.52		100.3695

				89.54		100.3747

				89.56		100.3747

				89.58		100.3747

				89.6		100.3695

				89.62		100.3747

				89.65		100.3747

				89.67		100.3747

				89.69		100.3747

				89.71		100.3747

				89.73		100.3747

				89.75		100.3747

				89.77		100.3747

				89.79		100.3747

				89.81		100.3747

				89.84		100.3747

				89.86		100.3747

				89.88		100.3747

				89.9		100.3747

				89.92		100.3747

				89.94		100.3747

				89.96		100.3747

				89.98		100.3747

				90		100.3747

				90.03		100.3747

				90.05		100.3747

				90.07		100.3747

				90.09		100.3747

				90.11		100.3747

				90.13		100.3747

				90.15		100.3747

				90.17		100.3747

				90.19		100.3799

				90.22		100.3799

				90.24		100.3747

				90.26		100.3747

				90.28		100.3799

				90.3		100.3747

				90.32		100.3747

				90.34		100.3747

				90.36		100.3747

				90.38		100.3747

				90.41		100.3747

				90.43		100.3747

				90.45		100.3747

				90.47		100.3747

				90.49		100.3747

				90.51		100.3747

				90.53		100.3747

				90.55		100.3747

				90.57		100.3747

				90.6		100.3747

				90.62		100.3747

				90.64		100.3747

				90.66		100.3747

				90.68		100.3747

				90.7		100.3747

				90.72		100.3747

				90.74		100.3747

				90.76		100.3747

				90.79		100.3747

				90.81		100.3747

				90.83		100.3747

				90.85		100.3747

				90.87		100.3747

				90.89		100.3747

				90.91		100.3747

				90.93		100.3747

				90.95		100.3695

				90.98		100.3695

				91		100.3695

				91.02		100.3695

				91.04		100.3695

				91.06		100.3747

				91.08		100.3747

				91.1		100.3747

				91.12		100.3747

				91.14		100.3747

				91.17		100.3747

				91.19		100.3747

				91.21		100.3747

				91.23		100.3747

				91.25		100.3747

				91.27		100.3747

				91.29		100.3747

				91.31		100.3747

				91.33		100.3747

				91.36		100.3747

				91.38		100.3747

				91.4		100.3695

				91.42		100.3747

				91.44		100.3695

				91.46		100.3695

				91.48		100.3695

				91.5		100.3747

				91.52		100.3747

				91.55		100.3747

				91.57		100.3695

				91.59		100.3695

				91.61		100.3695

				91.63		100.3695

				91.65		100.3695

				91.67		100.3695

				91.69		100.3695

				91.71		100.3695

				91.74		100.3747

				91.76		100.3695

				91.78		100.3695

				91.8		100.3695

				91.82		100.3695

				91.84		100.3695

				91.86		100.3695

				91.88		100.3695

				91.9		100.3695

				91.93		100.3695

				91.95		100.3695

				91.97		100.3695

				91.99		100.3695

				92.01		100.3695

				92.03		100.3695

				92.05		100.3695

				92.07		100.3695

				92.09		100.3695

				92.12		100.3695

				92.14		100.3695

				92.16		100.3695

				92.18		100.3695

				92.2		100.3695

				92.22		100.3695

				92.24		100.3695

				92.26		100.3695

				92.28		100.3695

				92.31		100.3695

				92.33		100.3695

				92.35		100.3695

				92.37		100.3695

				92.39		100.3695

				92.41		100.3695

				92.43		100.3695

				92.45		100.3695

				92.47		100.3695

				92.5		100.3695

				92.52		100.3695

				92.54		100.3695

				92.56		100.3695

				92.58		100.3695

				92.6		100.3695

				92.62		100.3695

				92.64		100.3695

				92.66		100.3695

				92.68		100.3695

				92.71		100.3695

				92.73		100.3695

				92.75		100.3695

				92.77		100.3695

				92.79		100.3695

				92.81		100.3695

				92.83		100.3695

				92.85		100.3695

				92.87		100.3695

				92.9		100.3695

				92.92		100.3695

				92.94		100.3695

				92.96		100.3695

				92.98		100.3695

				93		100.3695

				93.02		100.3695

				93.04		100.3695

				93.06		100.3695

				93.09		100.3695

				93.11		100.3695

				93.13		100.3747

				93.15		100.3747

				93.17		100.3747

				93.19		100.3695

				93.21		100.3747

				93.23		100.3747

				93.25		100.3747

				93.28		100.3695

				93.3		100.3695

				93.32		100.3695

				93.34		100.3695

				93.36		100.3695

				93.38		100.3695

				93.4		100.3695

				93.42		100.3695

				93.44		100.3695

				93.47		100.3695

				93.49		100.3695

				93.51		100.3695

				93.53		100.3747

				93.55		100.3747

				93.57		100.3747

				93.59		100.3695

				93.61		100.3747

				93.63		100.3747

				93.66		100.3747

				93.68		100.3747

				93.7		100.3747

				93.72		100.3747

				93.74		100.3747

				93.76		100.3747

				93.78		100.3747

				93.8		100.3747

				93.82		100.3695

				93.85		100.3695

				93.87		100.3695

				93.89		100.3695

				93.91		100.3695

				93.93		100.3695

				93.95		100.3695

				93.97		100.3695

				93.99		100.3695

				94.01		100.3695

				94.04		100.3695

				94.06		100.3747

				94.08		100.3747

				94.1		100.3747

				94.12		100.3747

				94.14		100.3747

				94.16		100.3747

				94.18		100.3747

				94.2		100.3695

				94.23		100.3695

				94.25		100.3695

				94.27		100.3695

				94.29		100.3695

				94.31		100.3695

				94.33		100.3695

				94.35		100.3695

				94.37		100.3695

				94.39		100.3695

				94.42		100.3695

				94.44		100.3695

				94.46		100.3695

				94.48		100.3695

				94.5		100.3695

				94.52		100.3695

				94.54		100.3695

				94.56		100.3695

				94.58		100.3747

				94.6		100.3695

				94.63		100.3695

				94.65		100.3695

				94.67		100.3695

				94.69		100.3747

				94.71		100.3695

				94.73		100.3747

				94.75		100.3747

				94.77		100.3695

				94.79		100.3695

				94.82		100.3695

				94.84		100.3695

				94.86		100.3695

				94.88		100.3695

				94.9		100.3695

				94.92		100.3695

				94.94		100.3695

				94.96		100.3695

				94.98		100.3747

				95.01		100.3747

				95.03		100.3747

				95.05		100.3747

				95.07		100.3747

				95.09		100.3747

				95.11		100.3747

				95.13		100.3747

				95.15		100.3747

				95.17		100.3747

				95.2		100.3695

				95.22		100.3747

				95.24		100.3695

				95.26		100.3695

				95.28		100.3695

				95.3		100.3695

				95.32		100.3695

				95.34		100.3695

				95.36		100.3695

				95.39		100.3695

				95.41		100.3695

				95.43		100.3695

				95.45		100.3695

				95.47		100.3695

				95.49		100.3695

				95.51		100.3695

				95.53		100.3695

				95.55		100.3695

				95.58		100.3695

				95.6		100.3695

				95.62		100.3695

				95.64		100.3695

				95.66		100.3695

				95.68		100.3695

				95.7		100.3695

				95.72		100.3695

				95.74		100.3643

				95.77		100.3643

				95.79		100.3643

				95.81		100.3643

				95.83		100.3643

				95.85		100.3643

				95.87		100.3643

				95.89		100.3643

				95.91		100.3643

				95.93		100.3643

				95.96		100.3643

				95.98		100.3643

				96		100.3643

				96.02		100.3643

				96.04		100.3643

				96.06		100.3643

				96.08		100.3643

				96.1		100.3695

				96.12		100.3643

				96.15		100.3643

				96.17		100.3643

				96.19		100.3643

				96.21		100.3643

				96.23		100.3643

				96.25		100.3643

				96.27		100.3643

				96.29		100.3643

				96.31		100.3695

				96.33		100.3643

				96.36		100.3643

				96.38		100.3643

				96.4		100.3643

				96.42		100.3643

				96.44		100.3695

				96.46		100.3643

				96.48		100.3643

				96.5		100.3695

				96.52		100.3695

				96.55		100.3695

				96.57		100.3695

				96.59		100.3695

				96.61		100.3695

				96.63		100.3695

				96.65		100.3695

				96.67		100.3695

				96.69		100.3695

				96.71		100.3695

				96.74		100.3695

				96.76		100.3643

				96.78		100.3643

				96.8		100.3643

				96.82		100.3643

				96.84		100.3643

				96.86		100.3643

				96.88		100.3695

				96.9		100.3695

				96.93		100.3643

				96.95		100.3695

				96.97		100.3695

				96.99		100.3695

				97.01		100.3695

				97.03		100.3695

				97.05		100.3695

				97.07		100.3695

				97.09		100.3695

				97.11		100.3695

				97.14		100.3695

				97.16		100.3643

				97.18		100.3695

				97.2		100.3695

				97.22		100.3695

				97.24		100.3695

				97.26		100.3695

				97.28		100.3695

				97.3		100.3695

				97.33		100.3695

				97.35		100.3695

				97.37		100.3695

				97.39		100.3695

				97.41		100.3695

				97.43		100.3695

				97.45		100.3695

				97.47		100.3747

				97.49		100.3747

				97.52		100.3747

				97.54		100.3747

				97.56		100.3747

				97.58		100.3747

				97.6		100.3747

				97.62		100.3747

				97.64		100.3747

				97.66		100.3747

				97.68		100.3695

				97.71		100.3747

				97.73		100.3747

				97.75		100.3747

				97.77		100.3695

				97.79		100.3747

				97.81		100.3747

				97.83		100.3747

				97.85		100.3747

				97.87		100.3747

				97.9		100.3747

				97.92		100.3747

				97.94		100.3747

				97.96		100.3747

				97.98		100.3747

				98		100.3747

				98.02		100.3747

				98.04		100.3747

				98.06		100.3747

				98.08		100.3747

				98.11		100.3747

				98.13		100.3747

				98.15		100.3747

				98.17		100.3747

				98.19		100.3747

				98.21		100.3747

				98.23		100.3747

				98.25		100.3747

				98.27		100.3747

				98.3		100.3747

				98.32		100.3747

				98.34		100.3747

				98.36		100.3747

				98.38		100.3747

				98.4		100.3747

				98.42		100.3747

				98.44		100.3747

				98.46		100.3747

				98.49		100.3747

				98.51		100.3799

				98.53		100.3747

				98.55		100.3799

				98.57		100.3747

				98.59		100.3747

				98.61		100.3747

				98.63		100.3747

				98.65		100.3747

				98.68		100.3747

				98.7		100.3747

				98.72		100.3747

				98.74		100.3747

				98.76		100.3747

				98.78		100.3747

				98.8		100.3747

				98.82		100.3747

				98.84		100.3747

				98.87		100.3747

				98.89		100.3747

				98.91		100.3747

				98.93		100.3747

				98.95		100.3799

				98.97		100.3799

				98.99		100.3747

				99.01		100.3747

				99.03		100.3747

				99.05		100.3799

				99.08		100.3747

				99.1		100.3747

				99.12		100.3799

				99.14		100.3747

				99.16		100.3799

				99.18		100.3799

				99.2		100.3799

				99.22		100.3799

				99.24		100.3799

				99.27		100.3799

				99.29		100.3799

				99.31		100.3799

				99.33		100.3799

				99.35		100.3799

				99.37		100.3799

				99.39		100.3799

				99.41		100.3799

				99.43		100.3799

				99.46		100.3799

				99.48		100.3799

				99.5		100.3799

				99.52		100.3747

				99.54		100.3747

				99.56		100.3747

				99.58		100.3747

				99.6		100.3747

				99.62		100.3747

				99.64		100.3747

				99.67		100.3747

				99.69		100.3747

				99.71		100.3747

				99.73		100.3747

				99.75		100.3747

				99.77		100.3747

				99.79		100.3747

				99.81		100.3747

				99.83		100.3747

				99.86		100.3747

				99.88		100.3747

				99.9		100.3747

				99.92		100.3747

				99.94		100.3747

				99.96		100.3747

				99.98		100.3747

				100		100.3747

				100.02		100.3747

				100.05		100.3747

				100.07		100.3799

				100.09		100.3799

				100.11		100.3799

				100.13		100.3799

				100.15		100.3747

				100.17		100.3747

				100.19		100.3747

				100.21		100.3799

				100.24		100.3799

				100.26		100.3799

				100.28		100.3799

				100.3		100.3799

				100.32		100.3799

				100.34		100.3799

				100.36		100.3799

				100.38		100.3747

				100.4		100.3799

				100.43		100.3747

				100.45		100.3799

				100.47		100.3747

				100.49		100.3747

				100.51		100.3747

				100.53		100.3747

				100.55		100.3747

				100.57		100.3747

				100.59		100.3747

				100.61		100.3747

				100.64		100.3747

				100.66		100.3799

				100.68		100.3747

				100.7		100.3799

				100.72		100.3799

				100.74		100.3799

				100.76		100.3799

				100.78		100.3799

				100.8		100.3799

				100.83		100.3799

				100.85		100.3799

				100.87		100.3799

				100.89		100.3799

				100.91		100.3799

				100.93		100.3799

				100.95		100.3799

				100.97		100.3799

				100.99		100.3799

				101.02		100.3799

				101.04		100.3799

				101.06		100.3799

				101.08		100.3799

				101.1		100.3799

				101.12		100.3799

				101.14		100.3799

				101.16		100.3799

				101.18		100.3799

				101.21		100.3799

				101.23		100.3799

				101.25		100.3747

				101.27		100.3747

				101.29		100.3747

				101.31		100.3747

				101.33		100.3747

				101.35		100.3747

				101.37		100.3799

				101.39		100.3799

				101.42		100.3747

				101.44		100.3747

				101.46		100.3747

				101.48		100.3747

				101.5		100.3747

				101.52		100.3747

				101.54		100.3747

				101.56		100.3747

				101.58		100.3747

				101.61		100.3799

				101.63		100.3799

				101.65		100.3799

				101.67		100.3747

				101.69		100.3799

				101.71		100.3799

				101.73		100.3799

				101.75		100.3747

				101.77		100.3747

				101.8		100.3747

				101.82		100.3747

				101.84		100.3747

				101.86		100.3747

				101.88		100.3747

				101.9		100.3747

				101.92		100.3747

				101.94		100.3747

				101.96		100.3747

				101.98		100.3747

				102.01		100.3747

				102.03		100.3747

				102.05		100.3747

				102.07		100.3747

				102.09		100.3695

				102.11		100.3695

				102.13		100.3695

				102.15		100.3695

				102.17		100.3695

				102.2		100.3695

				102.22		100.3695

				102.24		100.3695

				102.26		100.3695

				102.28		100.3695

				102.3		100.3695

				102.32		100.3695

				102.34		100.3695

				102.36		100.3695

				102.38		100.3695

				102.41		100.3695

				102.43		100.3695

				102.45		100.3695

				102.47		100.3643

				102.49		100.3643

				102.51		100.3643

				102.53		100.3643

				102.55		100.3643

				102.57		100.3643

				102.6		100.3643

				102.62		100.3643

				102.64		100.3643

				102.66		100.3643

				102.68		100.3643

				102.7		100.3643

				102.72		100.3643

				102.74		100.3643

				102.76		100.3643

				102.78		100.3643

				102.81		100.3643

				102.83		100.3643

				102.85		100.3643

				102.87		100.3643

				102.89		100.3643

				102.91		100.3643

				102.93		100.3591

				102.95		100.3591

				102.97		100.3591

				103		100.3591

				103.02		100.3591

				103.04		100.3591

				103.06		100.3591

				103.08		100.3591

				103.1		100.3591

				103.12		100.3591

				103.14		100.3591

				103.16		100.3591

				103.19		100.3591

				103.21		100.3591

				103.23		100.3591

				103.25		100.3591

				103.27		100.3591

				103.29		100.3591

				103.31		100.3591

				103.33		100.3591

				103.35		100.3591

				103.37		100.3591

				103.4		100.3591

				103.42		100.3591

				103.44		100.3591

				103.46		100.3591

				103.48		100.3591

				103.5		100.3591

				103.52		100.3591

				103.54		100.3591

				103.56		100.3591

				103.59		100.3591

				103.61		100.3591

				103.63		100.3591

				103.65		100.3591

				103.67		100.3591

				103.69		100.3591

				103.71		100.3539

				103.73		100.3591

				103.75		100.3591

				103.78		100.3539

				103.8		100.3591

				103.82		100.3591

				103.84		100.3591

				103.86		100.3591

				103.88		100.3591

				103.9		100.3591

				103.92		100.3591

				103.94		100.3591

				103.96		100.3591

				103.99		100.3591

				104.01		100.3591

				104.03		100.3591

				104.05		100.3591

				104.07		100.3591

				104.09		100.3591

				104.11		100.3591

				104.13		100.3591

				104.15		100.3591

				104.18		100.3591

				104.2		100.3591

				104.22		100.3591

				104.24		100.3591

				104.26		100.3591

				104.28		100.3591

				104.3		100.3591

				104.32		100.3591

				104.34		100.3591

				104.37		100.3591

				104.39		100.3591

				104.41		100.3591

				104.43		100.3591

				104.45		100.3591

				104.47		100.3591

				104.49		100.3591

				104.51		100.3591

				104.53		100.3591

				104.55		100.3591

				104.58		100.3591

				104.6		100.3591

				104.62		100.3591

				104.64		100.3591

				104.66		100.3591

				104.68		100.3591

				104.7		100.3591

				104.72		100.3591

				104.74		100.3591

				104.77		100.3591

				104.79		100.3591

				104.81		100.3643

				104.83		100.3643

				104.85		100.3591

				104.87		100.3643

				104.89		100.3591

				104.91		100.3591

				104.93		100.3591

				104.95		100.3643

				104.98		100.3643

				105		100.3591

				105.02		100.3643

				105.04		100.3643

				105.06		100.3643

				105.08		100.3643

				105.1		100.3643

				105.12		100.3643

				105.14		100.3643

				105.17		100.3643

				105.19		100.3643

				105.21		100.3643

				105.23		100.3643

				105.25		100.3643

				105.27		100.3643

				105.29		100.3643

				105.31		100.3643

				105.33		100.3643

				105.35		100.3643

				105.38		100.3643

				105.4		100.3643

				105.42		100.3643

				105.44		100.3643

				105.46		100.3643

				105.48		100.3695

				105.5		100.3695

				105.52		100.3695

				105.54		100.3695

				105.57		100.3643

				105.59		100.3643

				105.61		100.3643

				105.63		100.3643

				105.65		100.3643

				105.67		100.3643

				105.69		100.3643

				105.71		100.3643

				105.73		100.3643

				105.76		100.3643

				105.78		100.3643

				105.8		100.3643

				105.82		100.3643

				105.84		100.3643

				105.86		100.3643

				105.88		100.3643

				105.9		100.3643

				105.92		100.3643

				105.94		100.3643

				105.97		100.3643

				105.99		100.3643

				106.01		100.3643

				106.03		100.3643

				106.05		100.3643

				106.07		100.3643

				106.09		100.3643

				106.11		100.3643

				106.13		100.3643

				106.16		100.3643

				106.18		100.3643

				106.2		100.3643

				106.22		100.3695

				106.24		100.3643

				106.26		100.3643

				106.28		100.3643

				106.3		100.3643

				106.32		100.3643

				106.34		100.3643

				106.37		100.3643

				106.39		100.3643

				106.41		100.3643

				106.43		100.3643

				106.45		100.3643

				106.47		100.3643

				106.49		100.3643

				106.51		100.3643

				106.53		100.3643

				106.56		100.3643

				106.58		100.3643

				106.6		100.3643

				106.62		100.3643

				106.64		100.3643

				106.66		100.3643

				106.68		100.3643

				106.7		100.3643

				106.72		100.3643

				106.74		100.3643

				106.77		100.3643

				106.79		100.3643

				106.81		100.3643

				106.83		100.3643

				106.85		100.3643

				106.87		100.3643

				106.89		100.3643

				106.91		100.3643

				106.93		100.3643

				106.96		100.3643

				106.98		100.3643

				107		100.3643

				107.02		100.3643

				107.04		100.3643

				107.06		100.3643

				107.08		100.3643

				107.1		100.3643

				107.12		100.3643

				107.14		100.3643

				107.17		100.3643

				107.19		100.3643

				107.21		100.3643

				107.23		100.3643

				107.25		100.3643

				107.27		100.3643

				107.29		100.3643

				107.31		100.3643

				107.33		100.3643

				107.35		100.3695

				107.38		100.3695

				107.4		100.3695

				107.42		100.3695

				107.44		100.3695

				107.46		100.3695

				107.48		100.3695

				107.5		100.3695

				107.52		100.3695

				107.54		100.3695

				107.57		100.3643

				107.59		100.3643

				107.61		100.3695

				107.63		100.3695

				107.65		100.3695

				107.67		100.3695

				107.69		100.3695

				107.71		100.3695

				107.73		100.3695

				107.75		100.3695

				107.78		100.3695

				107.8		100.3695

				107.82		100.3695

				107.84		100.3695

				107.86		100.3695

				107.88		100.3695

				107.9		100.3747

				107.92		100.3695

				107.94		100.3695

				107.97		100.3695

				107.99		100.3695

				108.01		100.3695

				108.03		100.3695

				108.05		100.3695

				108.07		100.3695

				108.09		100.3695

				108.11		100.3695

				108.13		100.3695

				108.15		100.3695

				108.18		100.3695

				108.2		100.3695

				108.22		100.3695

				108.24		100.3695

				108.26		100.3695

				108.28		100.3695

				108.3		100.3695

				108.32		100.3747

				108.34		100.3695

				108.37		100.3695

				108.39		100.3695

				108.41		100.3695

				108.43		100.3747

				108.45		100.3695

				108.47		100.3695

				108.49		100.3695

				108.51		100.3695

				108.53		100.3695

				108.55		100.3695

				108.58		100.3695

				108.6		100.3695

				108.62		100.3695

				108.64		100.3695

				108.66		100.3695

				108.68		100.3695

				108.7		100.3695

				108.72		100.3695

				108.74		100.3695

				108.77		100.3695

				108.79		100.3695

				108.81		100.3695

				108.83		100.3695

				108.85		100.3695

				108.87		100.3695

				108.89		100.3695

				108.91		100.3643

				108.93		100.3695

				108.95		100.3695

				108.98		100.3643

				109		100.3643

				109.02		100.3643

				109.04		100.3643

				109.06		100.3643

				109.08		100.3643

				109.1		100.3643

				109.12		100.3643

				109.14		100.3643

				109.16		100.3643

				109.19		100.3643

				109.21		100.3643

				109.23		100.3643

				109.25		100.3643

				109.27		100.3643

				109.29		100.3643

				109.31		100.3643

				109.33		100.3643

				109.35		100.3591

				109.38		100.3591

				109.4		100.3591

				109.42		100.3591

				109.44		100.3591

				109.46		100.3591

				109.48		100.3591

				109.5		100.3591

				109.52		100.3539

				109.54		100.3539

				109.57		100.3539

				109.59		100.3539

				109.61		100.3539

				109.63		100.3539

				109.65		100.3539

				109.67		100.3539

				109.69		100.3539

				109.71		100.3539

				109.73		100.3539

				109.75		100.3539

				109.78		100.3539

				109.8		100.3539

				109.82		100.3539

				109.84		100.3539

				109.86		100.3539

				109.88		100.3539

				109.9		100.3486

				109.92		100.3486

				109.94		100.3486

				109.97		100.3486

				109.99		100.3486

				110.01		100.3486

				110.03		100.3486

				110.05		100.3486

				110.07		100.3486

				110.09		100.3486

				110.11		100.3486

				110.13		100.3486

				110.15		100.3486

				110.18		100.3486

				110.2		100.3486

				110.22		100.3486

				110.24		100.3486

				110.26		100.3486

				110.28		100.3486

				110.3		100.3486

				110.32		100.3486

				110.34		100.3486

				110.36		100.3486

				110.39		100.3486

				110.41		100.3486

				110.43		100.3486

				110.45		100.3486

				110.47		100.3486

				110.49		100.3486

				110.51		100.3486

				110.53		100.3486

				110.55		100.3486

				110.58		100.3486

				110.6		100.3486

				110.62		100.3486

				110.64		100.3486

				110.66		100.3486

				110.68		100.3486

				110.7		100.3486

				110.72		100.3486

				110.74		100.3486

				110.76		100.3486

				110.79		100.3486

				110.81		100.3486

				110.83		100.3486

				110.85		100.3486

				110.87		100.3486

				110.89		100.3486

				110.91		100.3486

				110.93		100.3486

				110.95		100.3486

				110.98		100.3486

				111		100.3486

				111.02		100.3486

				111.04		100.3486

				111.06		100.3486

				111.08		100.3486

				111.1		100.3486

				111.12		100.3486

				111.14		100.3486

				111.16		100.3486

				111.19		100.3486

				111.21		100.3486

				111.23		100.3539

				111.25		100.3486

				111.27		100.3486

				111.29		100.3486

				111.31		100.3539

				111.33		100.3539

				111.35		100.3539

				111.38		100.3539

				111.4		100.3591

				111.42		100.3539

				111.44		100.3539

				111.46		100.3591

				111.48		100.3539

				111.5		100.3591

				111.52		100.3539

				111.54		100.3539

				111.56		100.3539

				111.59		100.3539

				111.61		100.3539

				111.63		100.3591

				111.65		100.3539

				111.67		100.3591

				111.69		100.3591

				111.71		100.3591

				111.73		100.3591

				111.75		100.3539

				111.78		100.3539

				111.8		100.3539

				111.82		100.3539

				111.84		100.3539

				111.86		100.3539

				111.88		100.3539

				111.9		100.3539

				111.92		100.3539

				111.94		100.3539

				111.97		100.3539

				111.99		100.3591

				112.01		100.3591

				112.03		100.3539

				112.05		100.3591

				112.07		100.3591

				112.09		100.3591

				112.11		100.3591

				112.13		100.3591

				112.15		100.3591

				112.18		100.3591

				112.2		100.3591

				112.22		100.3591

				112.24		100.3591

				112.26		100.3591

				112.28		100.3591

				112.3		100.3591

				112.32		100.3591

				112.34		100.3591

				112.37		100.3539

				112.39		100.3591

				112.41		100.3591

				112.43		100.3591

				112.45		100.3591

				112.47		100.3591

				112.49		100.3591

				112.51		100.3591

				112.53		100.3591

				112.55		100.3591

				112.58		100.3591

				112.6		100.3591

				112.62		100.3591

				112.64		100.3591

				112.66		100.3591

				112.68		100.3591

				112.7		100.3539

				112.72		100.3539

				112.74		100.3539

				112.77		100.3591

				112.79		100.3539

				112.81		100.3591

				112.83		100.3591

				112.85		100.3591

				112.87		100.3539

				112.89		100.3591

				112.91		100.3591

				112.93		100.3591

				112.95		100.3539

				112.98		100.3539

				113		100.3539

				113.02		100.3539

				113.04		100.3539

				113.06		100.3539

				113.08		100.3539

				113.1		100.3539

				113.12		100.3539

				113.14		100.3539

				113.17		100.3539

				113.19		100.3539

				113.21		100.3539

				113.23		100.3539

				113.25		100.3539

				113.27		100.3591

				113.29		100.3539

				113.31		100.3591

				113.33		100.3539

				113.35		100.3539

				113.38		100.3539

				113.4		100.3539

				113.42		100.3486

				113.44		100.3539

				113.46		100.3539

				113.48		100.3539

				113.5		100.3539

				113.52		100.3539

				113.54		100.3539

				113.57		100.3486

				113.59		100.3486

				113.61		100.333

				113.63		100.3278

				113.65		100.3278

				113.67		100.3278

				113.69		100.3278

				113.71		100.3278

				113.73		100.3278

				113.76		100.3278

				113.78		100.333

				113.8		100.333

				113.82		100.333

				113.84		100.333

				113.86		100.3278

				113.88		100.3278

				113.9		100.3278

				113.92		100.3278

				113.94		100.3226

				113.97		100.3226

				113.99		100.3226

				114.01		100.3226

				114.03		100.3226

				114.05		100.3226

				114.07		100.3226

				114.09		100.3226

				114.11		100.3226

				114.13		100.3226

				114.16		100.3226

				114.18		100.3226

				114.2		100.3226

				114.22		100.3226

				114.24		100.3226

				114.26		100.3278

				114.28		100.3226

				114.3		100.3226

				114.32		100.3226

				114.34		100.3226

				114.37		100.3278

				114.39		100.3278

				114.41		100.3278

				114.43		100.3278

				114.45		100.3226

				114.47		100.3278

				114.49		100.3278

				114.51		100.3278

				114.53		100.3226

				114.55		100.3226

				114.58		100.3226

				114.6		100.3226

				114.62		100.3226

				114.64		100.3226

				114.66		100.3174

				114.68		100.3174

				114.7		100.3122

				114.72		100.3122

				114.74		100.3122

				114.77		100.3122

				114.79		100.3174

				114.81		100.3122

				114.83		100.3174

				114.85		100.3122

				114.87		100.3174

				114.89		100.3278

				114.91		100.3434

				114.93		100.3539

				114.95		100.3643

				114.98		100.3695

				115		100.3747

				115.02		100.3747

				115.04		100.3799

				115.06		100.3799

				115.08		100.3799

				115.1		100.3799

				115.12		100.3799

				115.14		100.3799

				115.16		100.3799

				115.19		100.3747

				115.21		100.3799

				115.23		100.3747

				115.25		100.3747

				115.27		100.3747

				115.29		100.3747

				115.31		100.3747

				115.33		100.3747

				115.35		100.3747

				115.38		100.3747

				115.4		100.3695

				115.42		100.3695

				115.44		100.3695

				115.46		100.3695

				115.48		100.3695

				115.5		100.3643

				115.52		100.3643

				115.54		100.3643

				115.56		100.3643

				115.59		100.3643

				115.61		100.3643

				115.63		100.3643

				115.65		100.3643

				115.67		100.3643

				115.69		100.3643

				115.71		100.3591

				115.73		100.3591

				115.75		100.3591

				115.78		100.3591

				115.8		100.3591

				115.82		100.3591

				115.84		100.3591

				115.86		100.3591

				115.88		100.3643

				115.9		100.3643

				115.92		100.3643

				115.94		100.3643

				115.96		100.3643

				115.99		100.3643

				116.01		100.3643

				116.03		100.3643

				116.05		100.3591

				116.07		100.3591

				116.09		100.3591

				116.11		100.3591

				116.13		100.3591

				116.15		100.3591

				116.18		100.3591

				116.2		100.3591

				116.22		100.3591

				116.24		100.3591

				116.26		100.3591

				116.28		100.3539

				116.3		100.3539

				116.32		100.3539

				116.34		100.3539

				116.37		100.3539

				116.39		100.3539

				116.41		100.3539

				116.43		100.3539

				116.45		100.3539

				116.47		100.3486

				116.49		100.3486

				116.51		100.3486

				116.53		100.3486

				116.55		100.3434

				116.58		100.3434

				116.6		100.3382

				116.62		100.3382

				116.64		100.3382

				116.66		100.3382

				116.68		100.3382

				116.7		100.3382

				116.72		100.3382

				116.74		100.3382

				116.76		100.3382

				116.79		100.3382

				116.81		100.333

				116.83		100.3382

				116.85		100.333

				116.87		100.333

				116.89		100.333

				116.91		100.333

				116.93		100.3382

				116.95		100.3382

				116.98		100.3382

				117		100.3382

				117.02		100.3382

				117.04		100.3382

				117.06		100.3382

				117.08		100.3382

				117.1		100.3382

				117.12		100.3382

				117.14		100.3382

				117.17		100.3382

				117.19		100.3382

				117.21		100.3382

				117.23		100.3382

				117.25		100.3382

				117.27		100.3382

				117.29		100.3382

				117.31		100.3382

				117.33		100.3382

				117.35		100.3382

				117.38		100.3382

				117.4		100.3382

				117.42		100.3382

				117.44		100.3382

				117.46		100.3382

				117.48		100.3382

				117.5		100.3382

				117.52		100.3382

				117.54		100.3382

				117.57		100.3382

				117.59		100.3382

				117.61		100.3382

				117.63		100.3382

				117.65		100.3382

				117.67		100.333

				117.69		100.333

				117.71		100.333

				117.73		100.333

				117.75		100.333

				117.78		100.333

				117.8		100.333

				117.82		100.333

				117.84		100.333

				117.86		100.333

				117.88		100.333

				117.9		100.333

				117.92		100.333

				117.94		100.333

				117.96		100.333

				117.99		100.333

				118.01		100.333

				118.03		100.333

				118.05		100.333

				118.07		100.333

				118.09		100.333

				118.11		100.333

				118.13		100.333

				118.15		100.333

				118.18		100.333

				118.2		100.3278

				118.22		100.3278

				118.24		100.3278

				118.26		100.3278

				118.28		100.3278

				118.3		100.3278

				118.32		100.3278

				118.34		100.3278

				118.36		100.3278

				118.39		100.3278

				118.41		100.3278

				118.43		100.3278

				118.45		100.3278

				118.47		100.3278

				118.49		100.3278

				118.51		100.3278

				118.53		100.3278

				118.55		100.3278

				118.58		100.3278

				118.6		100.3278

				118.62		100.3278

				118.64		100.3278

				118.66		100.3226

				118.68		100.3278

				118.7		100.3226

				118.72		100.3226

				118.74		100.3226

				118.76		100.3226

				118.79		100.3226

				118.81		100.3226

				118.83		100.3226

				118.85		100.3226

				118.87		100.3226

				118.89		100.3226

				118.91		100.3226

				118.93		100.3226

				118.95		100.3226

				118.98		100.3226

				119		100.3226

				119.02		100.3226

				119.04		100.3226

				119.06		100.3226

				119.08		100.3226

				119.1		100.3226

				119.12		100.3226

				119.14		100.3226

				119.16		100.3226

				119.19		100.3174

				119.21		100.3174

				119.23		100.3174

				119.25		100.3174

				119.27		100.3174

				119.29		100.3174

				119.31		100.3174

				119.33		100.3174

				119.35		100.3174

				119.37		100.3174

				119.4		100.3174

				119.42		100.3174

				119.44		100.3174

				119.46		100.3174

				119.48		100.3174

				119.5		100.3174

				119.52		100.3174

				119.54		100.3174

				119.56		100.3174

				119.59		100.3174

				119.61		100.3174

				119.63		100.3174

				119.65		100.3174

				119.67		100.3122

				119.69		100.3122

				119.71		100.3122

				119.73		100.3122

				119.75		100.3122

				119.77		100.3122

				119.8		100.3122

				119.82		100.3122

				119.84		100.3122

				119.86		100.3122

				119.88		100.3122

				119.9		100.3122

				119.92		100.3122

				119.94		100.3122

				119.96		100.3122

				119.99		100.3122

				120.01		100.3122

				120.03		100.3122

				120.05		100.3122

				120.07		100.307

				120.09		100.307

				120.11		100.307

				120.13		100.307

				120.15		100.307

				120.17		100.307

				120.2		100.307

				120.22		100.307

				120.24		100.307

				120.26		100.307

				120.28		100.307

				120.3		100.307

				120.32		100.307

				120.34		100.307

				120.36		100.307

				120.39		100.307

				120.41		100.307

				120.43		100.307

				120.45		100.307

				120.47		100.307

				120.49		100.307

				120.51		100.307

				120.53		100.307

				120.55		100.3018

				120.57		100.3018

				120.6		100.3018

				120.62		100.3018

				120.64		100.3018

				120.66		100.3018

				120.68		100.3018

				120.7		100.3018

				120.72		100.3018

				120.74		100.3018

				120.76		100.3018

				120.79		100.3018

				120.81		100.3018

				120.83		100.3018

				120.85		100.3018

				120.87		100.3018

				120.89		100.3018

				120.91		100.3018

				120.93		100.3018

				120.95		100.3018

				120.97		100.3018

				121		100.3018

				121.02		100.3018

				121.04		100.3018

				121.06		100.3018

				121.08		100.2966

				121.1		100.2966

				121.12		100.2966

				121.14		100.2966

				121.16		100.2966

				121.18		100.2966

				121.21		100.2966

				121.23		100.2966

				121.25		100.2966

				121.27		100.2966

				121.29		100.2966

				121.31		100.3018

				121.33		100.3018

				121.35		100.3018

				121.37		100.2966

				121.4		100.3018

				121.42		100.2966

				121.44		100.2966

				121.46		100.2966

				121.48		100.2966

				121.5		100.2966

				121.52		100.2966

				121.54		100.2966

				121.56		100.2966

				121.58		100.2966

				121.61		100.2966

				121.63		100.2966

				121.65		100.2966

				121.67		100.2966

				121.69		100.2966

				121.71		100.2966

				121.73		100.2914

				121.75		100.2914

				121.77		100.2966

				121.8		100.2966

				121.82		100.2914

				121.84		100.2914

				121.86		100.2914

				121.88		100.2914

				121.9		100.2914

				121.92		100.2914

				121.94		100.2862

				121.96		100.2914

				121.98		100.2966

				122.01		100.2966

				122.03		100.2966

				122.05		100.2914

				122.07		100.2966

				122.09		100.2966

				122.11		100.2966

				122.13		100.2966

				122.15		100.2966

				122.17		100.2966

				122.19		100.2966

				122.22		100.2966

				122.24		100.2966

				122.26		100.2966

				122.28		100.2966

				122.3		100.2966

				122.32		100.2966

				122.34		100.2966

				122.36		100.2966

				122.38		100.2966

				122.4		100.2966

				122.43		100.2966

				122.45		100.2966

				122.47		100.2966

				122.49		100.2966

				122.51		100.2966

				122.53		100.2966

				122.55		100.2966

				122.57		100.2966

				122.59		100.2966

				122.62		100.2966

				122.64		100.2966

				122.66		100.2966

				122.68		100.2966

				122.7		100.2966

				122.72		100.2966

				122.74		100.2966

				122.76		100.2966

				122.78		100.2966

				122.8		100.2966

				122.83		100.2966

				122.85		100.2966

				122.87		100.2966

				122.89		100.2914

				122.91		100.2966

				122.93		100.2966

				122.95		100.2914

				122.97		100.2914

				122.99		100.2966

				123.01		100.2966

				123.04		100.2966

				123.06		100.2966

				123.08		100.2966

				123.1		100.2966

				123.12		100.2966

				123.14		100.2966

				123.16		100.2966

				123.18		100.2914

				123.2		100.2966

				123.23		100.2914

				123.25		100.2914

				123.27		100.2914

				123.29		100.2914

				123.31		100.2914

				123.33		100.2914

				123.35		100.2914

				123.37		100.2914

				123.39		100.2862

				123.41		100.2862

				123.44		100.2862

				123.46		100.2862

				123.48		100.2914

				123.5		100.2914

				123.52		100.2914

				123.54		100.2914

				123.56		100.2914

				123.58		100.2914

				123.6		100.2914

				123.63		100.2914

				123.65		100.2914

				123.67		100.2914

				123.69		100.2914

				123.71		100.2914

				123.73		100.2862

				123.75		100.2862

				123.77		100.2914

				123.79		100.2862

				123.81		100.2862

				123.84		100.2862

				123.86		100.2862

				123.88		100.2862

				123.9		100.2862

				123.92		100.2862

				123.94		100.2862

				123.96		100.2862

				123.98		100.2862

				124		100.2914

				124.03		100.2914

				124.05		100.2862

				124.07		100.281

				124.09		100.2862

				124.11		100.281

				124.13		100.281

				124.15		100.281

				124.17		100.281

				124.19		100.281

				124.22		100.281

				124.24		100.281

				124.26		100.281

				124.28		100.281

				124.3		100.281

				124.32		100.281

				124.34		100.281

				124.36		100.281

				124.38		100.281

				124.4		100.281

				124.43		100.281

				124.45		100.281

				124.47		100.281

				124.49		100.281

				124.51		100.281

				124.53		100.281

				124.55		100.281

				124.57		100.281

				124.59		100.281

				124.62		100.281

				124.64		100.281

				124.66		100.281

				124.68		100.281

				124.7		100.281

				124.72		100.281

				124.74		100.281

				124.76		100.281

				124.78		100.281

				124.81		100.281

				124.83		100.281

				124.85		100.281

				124.87		100.281

				124.89		100.281

				124.91		100.281

				124.93		100.281

				124.95		100.281

				124.97		100.281

				124.99		100.281

				125.02		100.281

				125.04		100.281

				125.06		100.281

				125.08		100.281

				125.1		100.281

				125.12		100.281

				125.14		100.281

				125.16		100.281

				125.18		100.281

				125.21		100.281

				125.23		100.281

				125.25		100.281

				125.27		100.281

				125.29		100.281

				125.31		100.281

				125.33		100.281

				125.35		100.281

				125.37		100.281

				125.4		100.281

				125.42		100.281

				125.44		100.281

				125.46		100.281

				125.48		100.281

				125.5		100.281

				125.52		100.281

				125.54		100.281

				125.56		100.281

				125.59		100.281

				125.61		100.281

				125.63		100.2758

				125.65		100.2758

				125.67		100.281

				125.69		100.281

				125.71		100.2758

				125.73		100.2758

				125.75		100.2758

				125.78		100.2758

				125.8		100.2758

				125.82		100.2758

				125.84		100.2758

				125.86		100.2758

				125.88		100.2758

				125.9		100.2758

				125.92		100.2758

				125.94		100.2758

				125.97		100.2758

				125.99		100.281

				126.01		100.281

				126.03		100.2758

				126.05		100.281

				126.07		100.281

				126.09		100.2758

				126.11		100.2758

				126.13		100.2758

				126.15		100.2758

				126.18		100.2758

				126.2		100.2758

				126.22		100.2758

				126.24		100.2758

				126.26		100.2758

				126.28		100.2758

				126.3		100.2758

				126.32		100.2758

				126.34		100.2758

				126.37		100.2758

				126.39		100.2758

				126.41		100.2758

				126.43		100.2758

				126.45		100.2758

				126.47		100.2758

				126.49		100.2758

				126.51		100.2758

				126.53		100.2758

				126.56		100.2758

				126.58		100.2758

				126.6		100.2706

				126.62		100.2758

				126.64		100.2758

				126.66		100.2706

				126.68		100.2706

				126.7		100.2706

				126.72		100.2706

				126.75		100.2706

				126.77		100.2706

				126.79		100.2706

				126.81		100.2706

				126.83		100.2706

				126.85		100.2706

				126.87		100.2706

				126.89		100.2706

				126.91		100.2706

				126.94		100.2706

				126.96		100.2706

				126.98		100.2706

				127		100.2706

				127.02		100.2706

				127.04		100.2706

				127.06		100.2706

				127.08		100.2706

				127.1		100.2706

				127.12		100.2654

				127.15		100.2706

				127.17		100.2654

				127.19		100.2706

				127.21		100.2654

				127.23		100.2654

				127.25		100.2654

				127.27		100.2654

				127.29		100.2654

				127.31		100.2654

				127.34		100.2654

				127.36		100.2654

				127.38		100.2654

				127.4		100.2654

				127.42		100.2654

				127.44		100.2654

				127.46		100.2654

				127.48		100.2654

				127.5		100.2654

				127.53		100.2654

				127.55		100.2654

				127.57		100.2654

				127.59		100.2654

				127.61		100.2654

				127.63		100.2654

				127.65		100.2654

				127.67		100.2654

				127.69		100.2654

				127.72		100.2654

				127.74		100.2654

				127.76		100.2654

				127.78		100.2654

				127.8		100.2602

				127.82		100.2602

				127.84		100.2654

				127.86		100.2654

				127.88		100.2654

				127.91		100.2654

				127.93		100.2654

				127.95		100.2654

				127.97		100.2654

				127.99		100.2654

				128.01		100.2654

				128.03		100.2654

				128.05		100.2654

				128.07		100.2602

				128.09		100.2602

				128.12		100.2654

				128.14		100.2602

				128.16		100.2602

				128.18		100.2602

				128.2		100.2602

				128.22		100.2602

				128.24		100.2602

				128.26		100.2602

				128.28		100.2602

				128.31		100.2602

				128.33		100.2602

				128.35		100.2602

				128.37		100.2602

				128.39		100.2602

				128.41		100.2602

				128.43		100.2602

				128.45		100.2602

				128.47		100.2602

				128.5		100.2602

				128.52		100.2602

				128.54		100.2602

				128.56		100.2602

				128.58		100.2602

				128.6		100.255

				128.62		100.2602

				128.64		100.2602

				128.66		100.2602

				128.69		100.2602

				128.71		100.255

				128.73		100.255

				128.75		100.255

				128.77		100.255

				128.79		100.255

				128.81		100.255

				128.83		100.255

				128.85		100.255

				128.88		100.255

				128.9		100.255

				128.92		100.255

				128.94		100.255

				128.96		100.255

				128.98		100.255

				129		100.255

				129.02		100.255

				129.04		100.255

				129.07		100.255

				129.09		100.255

				129.11		100.255

				129.13		100.255

				129.15		100.255

				129.17		100.255

				129.19		100.255

				129.21		100.255

				129.23		100.255

				129.26		100.2498

				129.28		100.2498

				129.3		100.2498

				129.32		100.2498

				129.34		100.2498

				129.36		100.255

				129.38		100.2498

				129.4		100.2498

				129.42		100.2498

				129.45		100.2498

				129.47		100.2498

				129.49		100.2498

				129.51		100.2498

				129.53		100.2498

				129.55		100.2498

				129.57		100.2498

				129.59		100.2498

				129.61		100.2498

				129.63		100.2498

				129.66		100.2498

				129.68		100.2498

				129.7		100.2498

				129.72		100.2498

				129.74		100.2498

				129.76		100.2498

				129.78		100.2498

				129.8		100.2446

				129.82		100.2446

				129.85		100.2446

				129.87		100.2446

				129.89		100.2446

				129.91		100.2446

				129.93		100.2446

				129.95		100.2446

				129.97		100.2446

				129.99		100.2446

				130.01		100.2446

				130.04		100.2446

				130.06		100.2446

				130.08		100.2446

				130.1		100.2446

				130.12		100.2446

				130.14		100.2446

				130.16		100.2446

				130.18		100.2446

				130.2		100.2446

				130.23		100.2446

				130.25		100.2446

				130.27		100.2446

				130.29		100.2446

				130.31		100.2446

				130.33		100.2446

				130.35		100.2446

				130.37		100.2446

				130.4		100.2446

				130.42		100.2446

				130.44		100.2446

				130.46		100.2446

				130.48		100.2446

				130.5		100.2446

				130.52		100.2446

				130.54		100.2394

				130.56		100.2394

				130.59		100.2394

				130.61		100.2394

				130.63		100.2394

				130.65		100.2394

				130.67		100.2394

				130.69		100.2394

				130.71		100.2394

				130.73		100.2394

				130.75		100.2394

				130.78		100.2394

				130.8		100.2394

				130.82		100.2394

				130.84		100.2394

				130.86		100.2342

				130.88		100.2394

				130.9		100.2342

				130.92		100.2342

				130.94		100.2342

				130.97		100.2342

				130.99		100.2342

				131.01		100.2342

				131.03		100.2342

				131.05		100.2342

				131.07		100.2342

				131.09		100.2342

				131.11		100.2342

				131.13		100.229

				131.16		100.229

				131.18		100.229

				131.2		100.2342

				131.22		100.229

				131.24		100.229

				131.26		100.229

				131.28		100.229

				131.3		100.229

				131.32		100.229

				131.35		100.229

				131.37		100.229

				131.39		100.2238

				131.41		100.2238

				131.43		100.2238

				131.45		100.2238

				131.47		100.2238

				131.49		100.2238

				131.51		100.2238

				131.54		100.2238

				131.56		100.2238

				131.58		100.2238

				131.6		100.2238

				131.62		100.2186

				131.64		100.2238

				131.66		100.2238

				131.68		100.2238

				131.7		100.2186

				131.73		100.2186

				131.75		100.2186

				131.77		100.2186

				131.79		100.2186

				131.81		100.2186

				131.83		100.2186

				131.85		100.2186

				131.87		100.2186

				131.89		100.2186

				131.92		100.2186

				131.94		100.2186

				131.96		100.2186

				131.98		100.2186

				132		100.2186

				132.02		100.2186

				132.04		100.2134

				132.06		100.2134

				132.08		100.2134

				132.11		100.2134

				132.13		100.2134

				132.15		100.2134

				132.17		100.2134

				132.19		100.2134

				132.21		100.2081

				132.23		100.2134

				132.25		100.2081

				132.27		100.2081

				132.3		100.2081

				132.32		100.2081

				132.34		100.2081

				132.36		100.2081

				132.38		100.2081

				132.4		100.2081

				132.42		100.2029

				132.44		100.2029

				132.46		100.2029

				132.49		100.2029

				132.51		100.2029

				132.53		100.2029

				132.55		100.2029

				132.57		100.2029

				132.59		100.2029

				132.61		100.2029

				132.63		100.2029

				132.65		100.2029

				132.68		100.2029

				132.7		100.2029

				132.72		100.2029

				132.74		100.2029

				132.76		100.2029

				132.78		100.2029

				132.8		100.2029

				132.82		100.2029

				132.84		100.2029

				132.87		100.2029

				132.89		100.2029

				132.91		100.2029

				132.93		100.2029

				132.95		100.2029

				132.97		100.2029

				132.99		100.2029

				133.01		100.2029

				133.03		100.2029

				133.06		100.2029

				133.08		100.2029

				133.1		100.2029

				133.12		100.2029

				133.14		100.2029

				133.16		100.2029

				133.18		100.2029

				133.2		100.2029

				133.22		100.2029

				133.25		100.2029

				133.27		100.2029

				133.29		100.2029

				133.31		100.2029

				133.33		100.2029

				133.35		100.2029

				133.37		100.2029

				133.39		100.2029

				133.42		100.2029

				133.44		100.2029

				133.46		100.2029

				133.48		100.2029

				133.5		100.2029

				133.52		100.2029

				133.54		100.2029

				133.56		100.2081

				133.58		100.2029

				133.61		100.2081

				133.63		100.2081

				133.65		100.2029

				133.67		100.2081

				133.69		100.2081

				133.71		100.2081

				133.73		100.2081

				133.75		100.2081

				133.77		100.2081

				133.8		100.2081

				133.82		100.2029

				133.84		100.2029

				133.86		100.2029

				133.88		100.2029

				133.9		100.2029

				133.92		100.2029

				133.94		100.2029

				133.96		100.2029

				133.99		100.2029

				134.01		100.2029

				134.03		100.2029

				134.05		100.1977

				134.07		100.2029

				134.09		100.2029

				134.11		100.2029

				134.13		100.2029

				134.15		100.2029

				134.18		100.2029

				134.2		100.2029

				134.22		100.2029

				134.24		100.2029

				134.26		100.2029

				134.28		100.2029

				134.3		100.2029

				134.32		100.2029

				134.34		100.2029

				134.37		100.2029

				134.39		100.2029

				134.41		100.2029

				134.43		100.1977

				134.45		100.1925

				134.47		100.1977

				134.49		100.1925

				134.51		100.1977

				134.53		100.1977

				134.56		100.1925

				134.58		100.1925

				134.6		100.1925

				134.62		100.1925

				134.64		100.1925

				134.66		100.1925

				134.68		100.1873

				134.7		100.1873

				134.73		100.1873

				134.75		100.1873

				134.77		100.1873

				134.79		100.1873

				134.81		100.1873

				134.83		100.1873

				134.85		100.1873

				134.87		100.1873

				134.89		100.1873

				134.92		100.1873

				134.94		100.1873

				134.96		100.1821

				134.98		100.1873

				135		100.1821

				135.02		100.1821

				135.04		100.1821

				135.06		100.1821

				135.08		100.1821

				135.11		100.1769

				135.13		100.1769

				135.15		100.1769

				135.17		100.1769

				135.19		100.1769

				135.21		100.1717

				135.23		100.1717

				135.25		100.1717

				135.28		100.1665

				135.3		100.1717

				135.32		100.1665

				135.34		100.1665

				135.36		100.1665

				135.38		100.1613

				135.4		100.1613

				135.42		100.1613

				135.44		100.1613

				135.47		100.1665

				135.49		100.1665

				135.51		100.1665

				135.53		100.1665

				135.55		100.1665

				135.57		100.1665

				135.59		100.1613

				135.61		100.1613

				135.63		100.1613

				135.66		100.1613

				135.68		100.1613

				135.7		100.1561

				135.72		100.1613

				135.74		100.1561

				135.76		100.1561

				135.78		100.1561

				135.8		100.1561

				135.83		100.1561

				135.85		100.1561

				135.87		100.1561

				135.89		100.1561

				135.91		100.1561

				135.93		100.1561

				135.95		100.1561

				135.97		100.1509

				135.99		100.1509

				136.02		100.1509

				136.04		100.1509

				136.06		100.1509

				136.08		100.1509

				136.1		100.1509

				136.12		100.1509

				136.14		100.1509

				136.16		100.1509

				136.18		100.1509

				136.21		100.1457

				136.23		100.1457

				136.25		100.1457

				136.27		100.1457

				136.29		100.1457

				136.31		100.1457

				136.33		100.1457

				136.35		100.1457

				136.37		100.1405

				136.4		100.1405

				136.42		100.1405

				136.44		100.1405

				136.46		100.1405

				136.48		100.1405

				136.5		100.1405

				136.52		100.1405

				136.54		100.1457

				136.57		100.1405

				136.59		100.1405

				136.61		100.1405

				136.63		100.1405

				136.65		100.1405

				136.67		100.1405

				136.69		100.1405

				136.71		100.1405

				136.73		100.1405

				136.76		100.1405

				136.78		100.1405

				136.8		100.1405

				136.82		100.1405

				136.84		100.1405

				136.86		100.1353

				136.88		100.1353

				136.9		100.1405

				136.93		100.1353

				136.95		100.1353

				136.97		100.1353

				136.99		100.1353

				137.01		100.1353

				137.03		100.1353

				137.05		100.1353

				137.07		100.1353

				137.09		100.1353

				137.12		100.1353

				137.14		100.1301

				137.16		100.1301

				137.18		100.1301

				137.2		100.1301

				137.22		100.1301

				137.24		100.1301

				137.26		100.1301

				137.28		100.1301

				137.31		100.1249

				137.33		100.1249

				137.35		100.1249

				137.37		100.1249

				137.39		100.1249

				137.41		100.1249

				137.43		100.1249

				137.45		100.1249

				137.48		100.1249

				137.5		100.1249

				137.52		100.1249

				137.54		100.1249

				137.56		100.1249

				137.58		100.1249

				137.6		100.1249

				137.62		100.1249

				137.64		100.1249

				137.67		100.1249

				137.69		100.1249

				137.71		100.1249

				137.73		100.1249

				137.75		100.1249

				137.77		100.1249

				137.79		100.1249

				137.81		100.1197

				137.83		100.1249

				137.86		100.1197

				137.88		100.1197

				137.9		100.1197

				137.92		100.1197

				137.94		100.1197

				137.96		100.1197

				137.98		100.1197

				138		100.1197

				138.03		100.1197

				138.05		100.1197

				138.07		100.1197

				138.09		100.1197

				138.11		100.1197

				138.13		100.1197

				138.15		100.1197

				138.17		100.1145

				138.19		100.1145

				138.22		100.1145

				138.24		100.1145

				138.26		100.1145

				138.28		100.1145

				138.3		100.1145

				138.32		100.1145

				138.34		100.1145

				138.36		100.1145

				138.39		100.1145

				138.41		100.1145

				138.43		100.1145

				138.45		100.1145

				138.47		100.1145

				138.49		100.1145

				138.51		100.1145

				138.53		100.1145

				138.55		100.1145

				138.58		100.1145

				138.6		100.1145

				138.62		100.1145

				138.64		100.1145

				138.66		100.1145

				138.68		100.1145

				138.7		100.1145

				138.72		100.1145

				138.75		100.1093

				138.77		100.1093

				138.79		100.1093

				138.81		100.1093

				138.83		100.1093

				138.85		100.1093

				138.87		100.1093

				138.89		100.1093

				138.91		100.1093

				138.94		100.1093

				138.96		100.1093

				138.98		100.1093

				139		100.1093

				139.02		100.1093

				139.04		100.1093

				139.06		100.1093

				139.08		100.1041

				139.11		100.1093

				139.13		100.1093

				139.15		100.1093

				139.17		100.1093

				139.19		100.1093

				139.21		100.1093

				139.23		100.1093

				139.25		100.1041

				139.27		100.1041

				139.3		100.1041

				139.32		100.1041

				139.34		100.1041

				139.36		100.1041

				139.38		100.1041

				139.4		100.1041

				139.42		100.0989

				139.44		100.0989

				139.46		100.0989

				139.49		100.0989

				139.51		100.0989

				139.53		100.1041

				139.55		100.0989

				139.57		100.0989

				139.59		100.0989

				139.61		100.0989

				139.63		100.0989

				139.66		100.0989

				139.68		100.0989

				139.7		100.0989

				139.72		100.0989

				139.74		100.0989

				139.76		100.0989

				139.78		100.0937

				139.8		100.0937

				139.82		100.0937

				139.85		100.0937

				139.87		100.0937

				139.89		100.0937

				139.91		100.0937

				139.93		100.0937

				139.95		100.0937

				139.97		100.0937

				139.99		100.0937

				140.02		100.0885

				140.04		100.0937

				140.06		100.0885

				140.08		100.0885

				140.1		100.0885

				140.12		100.0885

				140.14		100.0885

				140.16		100.0885

				140.19		100.0885

				140.21		100.0885

				140.23		100.0885

				140.25		100.0885

				140.27		100.0885

				140.29		100.0885

				140.31		100.0833

				140.33		100.0833

				140.35		100.0833

				140.38		100.0833

				140.4		100.0833

				140.42		100.0833

				140.44		100.0833

				140.46		100.0833

				140.48		100.0833

				140.5		100.0781

				140.52		100.0781

				140.55		100.0781

				140.57		100.0781

				140.59		100.0781

				140.61		100.0781

				140.63		100.0781

				140.65		100.0781

				140.67		100.0781

				140.69		100.0729

				140.72		100.0781

				140.74		100.0729

				140.76		100.0729

				140.78		100.0729

				140.8		100.0729

				140.82		100.0729

				140.84		100.0729

				140.86		100.0729

				140.88		100.0729

				140.91		100.0676

				140.93		100.0676

				140.95		100.0676

				140.97		100.0676

				140.99		100.0676

				141.01		100.0676

				141.03		100.0676

				141.05		100.0624

				141.08		100.0624

				141.1		100.0624

				141.12		100.0624

				141.14		100.0624

				141.16		100.0624

				141.18		100.0624

				141.2		100.0624

				141.22		100.0624

				141.24		100.0624

				141.27		100.0572

				141.29		100.0572

				141.31		100.0572

				141.33		100.0624

				141.35		100.0572

				141.37		100.0572

				141.39		100.0572

				141.41		100.0572

				141.44		100.0572

				141.46		100.0572

				141.48		100.0572

				141.5		100.0572

				141.52		100.0572

				141.54		100.0572

				141.56		100.0572

				141.58		100.0572

				141.6		100.0572

				141.63		100.052

				141.65		100.052

				141.67		100.052

				141.69		100.052

				141.71		100.052

				141.73		100.052

				141.75		100.052

				141.77		100.052

				141.8		100.052

				141.82		100.052

				141.84		100.052

				141.86		100.052

				141.88		100.0468

				141.9		100.0468

				141.92		100.0468

				141.94		100.0468

				141.97		100.0468

				141.99		100.0468

				142.01		100.0468

				142.03		100.0468

				142.05		100.0468

				142.07		100.0468

				142.09		100.0468

				142.11		100.0468

				142.13		100.0468

				142.16		100.0468

				142.18		100.0468

				142.2		100.0468

				142.22		100.0416

				142.24		100.0416

				142.26		100.0416

				142.28		100.0416

				142.3		100.0416

				142.33		100.0416

				142.35		100.0416

				142.37		100.0364

				142.39		100.0364

				142.41		100.0416

				142.43		100.0364

				142.45		100.0364

				142.47		100.0364

				142.5		100.0364

				142.52		100.0364

				142.54		100.0364

				142.56		100.0364

				142.58		100.0364

				142.6		100.0364

				142.62		100.0364

				142.64		100.0364

				142.66		100.0312

				142.69		100.0312

				142.71		100.0312

				142.73		100.0312

				142.75		100.0312

				142.77		100.0312

				142.79		100.0312

				142.81		100.0312

				142.83		100.0312

				142.86		100.0312

				142.88		100.0312

				142.9		100.0312

				142.92		100.026

				142.94		100.026

				142.96		100.026

				142.98		100.0312

				143		100.026

				143.03		100.026

				143.05		100.026

				143.07		100.026

				143.09		100.026

				143.11		100.026

				143.13		100.026

				143.15		100.0208

				143.17		100.0208

				143.19		100.0208

				143.22		100.0208

				143.24		100.0208

				143.26		100.0208

				143.28		100.0208

				143.3		100.0208

				143.32		100.0156

				143.34		100.0156

				143.36		100.0156

				143.39		100.0156

				143.41		100.0156

				143.43		100.0156

				143.45		100.0156

				143.47		100.0104

				143.49		100.0104

				143.51		100.0104

				143.53		100.0104

				143.56		100.0104

				143.58		100.0104

				143.6		100.0104

				143.62		100.0052

				143.64		100.0052

				143.66		100.0052

				143.68		100.0052

				143.7		100.0052

				143.72		100.0052

				143.75		100.0052

				143.77		100.0052

				143.79		100.0052

				143.81		100.0052

				143.83		100.0052

				143.85		100

				143.87		100

				143.89		100

				143.92		100

				143.94		100

				143.96		100

				143.98		100

				144		100

				144.02		100

				144.04		100

				144.06		100

				144.09		100

				144.11		99.9948

				144.13		99.9948

				144.15		99.9948

				144.17		99.9948

				144.19		99.9948

				144.21		99.9948

				144.23		99.9948

				144.25		99.98959

				144.28		99.98959

				144.3		99.98959

				144.32		99.98959

				144.34		99.98959

				144.36		99.98959

				144.38		99.98959

				144.4		99.98959

				144.42		99.98959

				144.45		99.98959

				144.47		99.98959

				144.49		99.98959

				144.51		99.98439

				144.53		99.98439

				144.55		99.98439

				144.57		99.98439

				144.59		99.98439

				144.62		99.98439

				144.64		99.98439

				144.66		99.98439

				144.68		99.97919

				144.7		99.97919

				144.72		99.97919

				144.74		99.97919

				144.76		99.97919

				144.78		99.97919

				144.81		99.97919

				144.83		99.97919

				144.85		99.97398

				144.87		99.97398

				144.89		99.97398

				144.91		99.97398

				144.93		99.97398

				144.95		99.97398

				144.98		99.97398

				145		99.97398

				145.02		99.97398

				145.04		99.97398

				145.06		99.97398

				145.08		99.97398

				145.1		99.97398

				145.12		99.97398

				145.15		99.96878

				145.17		99.96878

				145.19		99.96878

				145.21		99.96878

				145.23		99.96878

				145.25		99.96878

				145.27		99.96357

				145.29		99.96357

				145.32		99.96357

				145.34		99.96357

				145.36		99.96357

				145.38		99.96357

				145.4		99.96357

				145.42		99.95837

				145.44		99.95837

				145.46		99.95837

				145.48		99.95837

				145.51		99.95837

				145.53		99.95837

				145.55		99.95837

				145.57		99.95837

				145.59		99.95837

				145.61		99.95317

				145.63		99.95837

				145.65		99.95317

				145.68		99.95317

				145.7		99.95317

				145.72		99.95317

				145.74		99.94796

				145.76		99.94796

				145.78		99.94796

				145.8		99.94796

				145.82		99.94796

				145.85		99.94796

				145.87		99.94276

				145.89		99.94276

				145.91		99.94276

				145.93		99.94276

				145.95		99.94276

				145.97		99.94276

				145.99		99.93756

				146.02		99.93756

				146.04		99.93756

				146.06		99.93756

				146.08		99.93756

				146.1		99.93235

				146.12		99.93756

				146.14		99.93235

				146.16		99.93235

				146.19		99.93235

				146.21		99.93235

				146.23		99.93235

				146.25		99.93235

				146.27		99.92715

				146.29		99.92715

				146.31		99.92715

				146.33		99.92715

				146.35		99.92715

				146.38		99.92715

				146.4		99.92715

				146.42		99.92194

				146.44		99.92194

				146.46		99.92194

				146.48		99.92194

				146.5		99.92194

				146.52		99.92194

				146.55		99.92194

				146.57		99.92194

				146.59		99.92194

				146.61		99.92194

				146.63		99.92194

				146.65		99.92194

				146.67		99.91674

				146.69		99.91674

				146.72		99.91674

				146.74		99.91674

				146.76		99.91674

				146.78		99.91674

				146.8		99.91674

				146.82		99.91674

				146.84		99.91674

				146.86		99.91154

				146.88		99.91154

				146.91		99.91154

				146.93		99.91154

				146.95		99.91154

				146.97		99.91154

				146.99		99.91154

				147.01		99.90633

				147.03		99.90633

				147.05		99.90633

				147.08		99.90633

				147.1		99.90633

				147.12		99.90633

				147.14		99.90633

				147.16		99.90633

				147.18		99.90633

				147.2		99.90113

				147.22		99.90113

				147.25		99.90113

				147.27		99.90113

				147.29		99.90113

				147.31		99.90113

				147.33		99.89593

				147.35		99.89593

				147.37		99.89593

				147.39		99.89593

				147.42		99.89593

				147.44		99.89593

				147.46		99.89593

				147.48		99.89072

				147.5		99.89072

				147.52		99.89072

				147.54		99.89072

				147.56		99.89072

				147.59		99.89072

				147.61		99.89072

				147.63		99.89072

				147.65		99.88552

				147.67		99.88552

				147.69		99.88552

				147.71		99.88552

				147.73		99.88552

				147.76		99.88552

				147.78		99.88552

				147.8		99.88552

				147.82		99.88552

				147.84		99.88552

				147.86		99.88031

				147.88		99.88031

				147.9		99.88031

				147.92		99.88031

				147.95		99.87511

				147.97		99.88031

				147.99		99.87511

				148.01		99.87511

				148.03		99.87511

				148.05		99.86991

				148.07		99.86991

				148.09		99.86991

				148.12		99.86991

				148.14		99.8647

				148.16		99.8647

				148.18		99.8647

				148.2		99.8647

				148.22		99.8647

				148.24		99.8647

				148.26		99.8647

				148.29		99.8595

				148.31		99.8595

				148.33		99.8595

				148.35		99.8595

				148.37		99.8543

				148.39		99.8543

				148.41		99.8543

				148.43		99.8543

				148.46		99.8543

				148.48		99.8543

				148.5		99.8543

				148.52		99.84909

				148.54		99.8543

				148.56		99.8543

				148.58		99.84909

				148.6		99.84909

				148.63		99.84909

				148.65		99.84909

				148.67		99.84909

				148.69		99.84389

				148.71		99.84909

				148.73		99.84389

				148.75		99.84389

				148.77		99.84389

				148.8		99.84389

				148.82		99.84389

				148.84		99.83868

				148.86		99.83868

				148.88		99.83868

				148.9		99.83868

				148.92		99.83868

				148.94		99.83868

				148.96		99.83868

				148.99		99.83348

				149.01		99.83348

				149.03		99.83348

				149.05		99.83348

				149.07		99.83348

				149.09		99.83348

				149.11		99.83348

				149.13		99.82828

				149.16		99.82828

				149.18		99.82828

				149.2		99.82828

				149.22		99.82828

				149.24		99.82828

				149.26		99.82307

				149.28		99.82307

				149.3		99.82307

				149.33		99.82307

				149.35		99.82307

				149.37		99.82307

				149.39		99.82307

				149.41		99.81787

				149.43		99.81787

				149.45		99.81787

				149.47		99.81787

				149.5		99.81787

				149.52		99.81787

				149.54		99.81787

				149.56		99.81787

				149.58		99.81267

				149.6		99.81267

				149.62		99.81267

				149.64		99.81267

				149.66		99.81267

				149.69		99.81267

				149.71		99.81267

				149.73		99.80746

				149.75		99.80746

				149.77		99.80746

				149.79		99.80746

				149.81		99.80746

				149.83		99.80746

				149.86		99.80226

				149.88		99.80226

				149.9		99.80226

				149.92		99.80226

				149.94		99.80226

				149.96		99.80226

				149.98		99.79705

				150		99.79705

				150.03		99.79705

				150.05		99.79185

				150.07		99.79185

				150.09		99.79185

				150.11		99.79185

				150.13		99.79185

				150.15		99.79185

				150.17		99.79185

				150.19		99.79185

				150.22		99.79185

				150.24		99.78665

				150.26		99.78665

				150.28		99.78665

				150.3		99.78665

				150.32		99.78665

				150.34		99.78665

				150.36		99.78144

				150.39		99.78144

				150.41		99.78144

				150.43		99.78144

				150.45		99.78144

				150.47		99.77624

				150.49		99.78144

				150.51		99.78144

				150.53		99.77624

				150.56		99.77624

				150.58		99.77624

				150.6		99.77624

				150.62		99.77624

				150.64		99.77104

				150.66		99.77104

				150.68		99.77104

				150.7		99.77104

				150.72		99.76583

				150.75		99.76583

				150.77		99.76583

				150.79		99.76583

				150.81		99.76583

				150.83		99.76583

				150.85		99.76583

				150.87		99.76583

				150.89		99.76583

				150.92		99.76583

				150.94		99.76583

				150.96		99.76583

				150.98		99.76063

				151		99.76063

				151.02		99.76063

				151.04		99.75542

				151.06		99.75542

				151.09		99.76063

				151.11		99.75542

				151.13		99.75542

				151.15		99.75542

				151.17		99.75542

				151.19		99.75022

				151.21		99.75022

				151.23		99.75022

				151.26		99.75022

				151.28		99.75022

				151.3		99.75022

				151.32		99.74502

				151.34		99.74502

				151.36		99.74502

				151.38		99.74502

				151.4		99.74502

				151.42		99.73981

				151.45		99.73981

				151.47		99.73981

				151.49		99.73981

				151.51		99.73981

				151.53		99.73981

				151.55		99.73461

				151.57		99.73461

				151.59		99.73461

				151.62		99.73461

				151.64		99.73461

				151.66		99.73461

				151.68		99.72941

				151.7		99.72941

				151.72		99.73461

				151.74		99.72941

				151.76		99.72941

				151.78		99.72941

				151.81		99.72941

				151.83		99.72941

				151.85		99.7242

				151.87		99.7242

				151.89		99.7242

				151.91		99.719

				151.93		99.719

				151.95		99.719

				151.98		99.719

				152		99.719

				152.02		99.719

				152.04		99.7138

				152.06		99.7138

				152.08		99.70859

				152.1		99.7138

				152.12		99.70859

				152.14		99.70859

				152.17		99.70859

				152.19		99.70859

				152.21		99.70859

				152.23		99.70859

				152.25		99.70339

				152.27		99.70339

				152.29		99.70339

				152.31		99.70339

				152.34		99.69818

				152.36		99.69818

				152.38		99.69818

				152.4		99.69818

				152.42		99.69818

				152.44		99.69298

				152.46		99.69298

				152.48		99.69298

				152.51		99.69298

				152.53		99.68778

				152.55		99.68778

				152.57		99.68778

				152.59		99.68778

				152.61		99.68778

				152.63		99.68778

				152.65		99.68778

				152.67		99.68778

				152.7		99.68778

				152.72		99.68257

				152.74		99.68257

				152.76		99.68257

				152.78		99.68257

				152.8		99.68257

				152.82		99.68257

				152.84		99.67737

				152.87		99.67737

				152.89		99.67737

				152.91		99.67737

				152.93		99.67217

				152.95		99.67217

				152.97		99.67217

				152.99		99.67217

				153.01		99.66696

				153.03		99.66696

				153.06		99.66696

				153.08		99.66696

				153.1		99.66176

				153.12		99.66176

				153.14		99.66176

				153.16		99.66176

				153.18		99.66176

				153.2		99.66176

				153.23		99.66176

				153.25		99.65655

				153.27		99.65655

				153.29		99.65655

				153.31		99.65655

				153.33		99.65655

				153.35		99.65135

				153.37		99.65135

				153.39		99.65135

				153.42		99.64615

				153.44		99.64615

				153.46		99.64615

				153.48		99.64615

				153.5		99.64094

				153.52		99.64094

				153.54		99.64094

				153.56		99.64094

				153.59		99.64094

				153.61		99.64094

				153.63		99.64094

				153.65		99.63574

				153.67		99.63574

				153.69		99.63574

				153.71		99.63574

				153.73		99.63574

				153.75		99.63054

				153.78		99.63054

				153.8		99.63054

				153.82		99.63054

				153.84		99.63054

				153.86		99.62533

				153.88		99.62533

				153.9		99.62013

				153.92		99.62013

				153.95		99.62013

				153.97		99.62013

				153.99		99.61492

				154.01		99.61492

				154.03		99.61492

				154.05		99.61492

				154.07		99.60972

				154.09		99.60972

				154.11		99.60972

				154.14		99.60972

				154.16		99.60972

				154.18		99.60972

				154.2		99.60972

				154.22		99.60452

				154.24		99.60452

				154.26		99.60972

				154.28		99.60972

				154.31		99.60452

				154.33		99.60452

				154.35		99.60452

				154.37		99.60452

				154.39		99.59931

				154.41		99.59931

				154.43		99.59931

				154.45		99.59931

				154.47		99.59931

				154.5		99.59411

				154.52		99.59411

				154.54		99.59411

				154.56		99.59411

				154.58		99.59411

				154.6		99.59411

				154.62		99.59411

				154.64		99.58891

				154.67		99.58891

				154.69		99.58891

				154.71		99.58891

				154.73		99.58891

				154.75		99.58891

				154.77		99.5837

				154.79		99.5837

				154.81		99.5837

				154.83		99.5837

				154.86		99.5837

				154.88		99.5837

				154.9		99.5785

				154.92		99.5785

				154.94		99.5785

				154.96		99.5785

				154.98		99.5785

				155		99.57329

				155.03		99.57329

				155.05		99.57329

				155.07		99.56809

				155.09		99.56809

				155.11		99.56809

				155.13		99.56809

				155.15		99.56809

				155.17		99.56809

				155.19		99.56809

				155.22		99.56809

				155.24		99.56809

				155.26		99.56809

				155.28		99.56809

				155.3		99.56809

				155.32		99.56289

				155.34		99.56289

				155.36		99.56289

				155.39		99.56289

				155.41		99.55768

				155.43		99.55768

				155.45		99.55768

				155.47		99.55768

				155.49		99.55768

				155.51		99.55248

				155.53		99.55248

				155.55		99.54728

				155.58		99.54728

				155.6		99.54728

				155.62		99.54728

				155.64		99.54728

				155.66		99.54728

				155.68		99.54728

				155.7		99.54728

				155.72		99.54728

				155.75		99.54207

				155.77		99.54207

				155.79		99.54207

				155.81		99.54207

				155.83		99.54207

				155.85		99.53687

				155.87		99.53687

				155.89		99.53687

				155.92		99.53166

				155.94		99.53166

				155.96		99.53166

				155.98		99.53166

				156		99.52646

				156.02		99.52646

				156.04		99.52646

				156.06		99.52646

				156.08		99.52646

				156.11		99.52646

				156.13		99.52126

				156.15		99.52126

				156.17		99.52126

				156.19		99.52126

				156.21		99.52126

				156.23		99.52126

				156.25		99.52126

				156.27		99.52126

				156.3		99.51605

				156.32		99.51605

				156.34		99.51605

				156.36		99.51085

				156.38		99.51605

				156.4		99.51085

				156.42		99.51085

				156.44		99.51085

				156.47		99.51085

				156.49		99.50565

				156.51		99.50565

				156.53		99.50565

				156.55		99.50565

				156.57		99.50044

				156.59		99.50044

				156.61		99.50044

				156.63		99.49524

				156.66		99.50044

				156.68		99.49524

				156.7		99.49524

				156.72		99.49524

				156.74		99.49003

				156.76		99.49003

				156.78		99.49003

				156.8		99.48483

				156.82		99.48483

				156.85		99.48483

				156.87		99.48483

				156.89		99.47963

				156.91		99.48483

				156.93		99.47963

				156.95		99.47963

				156.97		99.47963

				156.99		99.47963

				157.02		99.47442

				157.04		99.47442

				157.06		99.46922

				157.08		99.46922

				157.1		99.46922

				157.12		99.46922

				157.14		99.46402

				157.16		99.46402

				157.18		99.45881

				157.21		99.45881

				157.23		99.45361

				157.25		99.45361

				157.27		99.45361

				157.29		99.45361

				157.31		99.44841

				157.33		99.44841

				157.35		99.4432

				157.37		99.44841

				157.4		99.4432

				157.42		99.4432

				157.44		99.4432

				157.46		99.438

				157.48		99.438

				157.5		99.43279

				157.52		99.43279

				157.54		99.42759

				157.57		99.42759

				157.59		99.42759

				157.61		99.42759

				157.63		99.42239

				157.65		99.42239

				157.67		99.42239

				157.69		99.41718

				157.71		99.41718

				157.73		99.41718

				157.76		99.41718

				157.78		99.41198

				157.8		99.41198

				157.82		99.41198

				157.84		99.41198

				157.86		99.41198

				157.88		99.41198

				157.9		99.41198

				157.92		99.40678

				157.95		99.40678

				157.97		99.40678

				157.99		99.40678

				158.01		99.40678

				158.03		99.40157

				158.05		99.40678

				158.07		99.40157

				158.09		99.40157

				158.11		99.40157

				158.14		99.40157

				158.16		99.40157

				158.18		99.39637

				158.2		99.39637

				158.22		99.39637

				158.24		99.39637

				158.26		99.39637

				158.28		99.39116

				158.3		99.39116

				158.33		99.39637

				158.35		99.39116

				158.37		99.39116

				158.39		99.39116

				158.41		99.39116

				158.43		99.39116

				158.45		99.38596

				158.47		99.38596

				158.49		99.38596

				158.52		99.38596

				158.54		99.38596

				158.56		99.38076

				158.58		99.38076

				158.6		99.38076

				158.62		99.38076

				158.64		99.37555

				158.66		99.37555

				158.69		99.37555

				158.71		99.37555

				158.73		99.37035

				158.75		99.37035

				158.77		99.36515

				158.79		99.36515

				158.81		99.35994

				158.83		99.35994

				158.85		99.35994

				158.88		99.35474

				158.9		99.34953

				158.92		99.34953

				158.94		99.34953

				158.96		99.34433

				158.98		99.33913

				159		99.33913

				159.02		99.33913

				159.04		99.33392

				159.07		99.32872

				159.09		99.32872

				159.11		99.32872

				159.13		99.32872

				159.15		99.32352

				159.17		99.32352

				159.19		99.31831

				159.21		99.31831

				159.23		99.31311

				159.26		99.31311

				159.28		99.31311

				159.3		99.31311

				159.32		99.31311

				159.34		99.31311

				159.36		99.3079

				159.38		99.3079

				159.4		99.3027

				159.42		99.3027

				159.45		99.2975

				159.47		99.2975

				159.49		99.2975

				159.51		99.2975

				159.53		99.29229

				159.55		99.29229

				159.57		99.29229

				159.59		99.29229

				159.61		99.29229

				159.64		99.28709

				159.66		99.28709

				159.68		99.28709

				159.7		99.28709

				159.72		99.28709

				159.74		99.28189

				159.76		99.28189

				159.78		99.28189

				159.8		99.28189

				159.83		99.27668

				159.85		99.27668

				159.87		99.27148

				159.89		99.27148

				159.91		99.27148

				159.93		99.26627

				159.95		99.26627

				159.97		99.26627

				159.99		99.26107

				160.02		99.26627

				160.04		99.26107

				160.06		99.25587

				160.08		99.25587

				160.1		99.25587

				160.12		99.25066

				160.14		99.25066

				160.16		99.25066

				160.19		99.25066

				160.21		99.24546

				160.23		99.24546

				160.25		99.24546

				160.27		99.24026

				160.29		99.24026

				160.31		99.23505

				160.33		99.23505

				160.35		99.23505

				160.38		99.23505

				160.4		99.22985

				160.42		99.22985

				160.44		99.22985

				160.46		99.22985

				160.48		99.22464

				160.5		99.22464

				160.52		99.22464

				160.54		99.22464

				160.57		99.22464

				160.59		99.21944

				160.61		99.21944

				160.63		99.21944

				160.65		99.21944

				160.67		99.21424

				160.69		99.21424

				160.71		99.21424

				160.73		99.20903

				160.75		99.20903

				160.78		99.20903

				160.8		99.20383

				160.82		99.20383

				160.84		99.20383

				160.86		99.20383

				160.88		99.19863

				160.9		99.19863

				160.92		99.19342

				160.94		99.19342

				160.97		99.19863

				160.99		99.19342

				161.01		99.19342

				161.03		99.19342

				161.05		99.18822

				161.07		99.18822

				161.09		99.18822

				161.11		99.18822

				161.13		99.18822

				161.16		99.18302

				161.18		99.18302

				161.2		99.17781

				161.22		99.17781

				161.24		99.17261

				161.26		99.17261

				161.28		99.17261

				161.3		99.1674

				161.32		99.1674

				161.35		99.1622

				161.37		99.1622

				161.39		99.157

				161.41		99.157

				161.43		99.157

				161.45		99.15179

				161.47		99.15179

				161.49		99.15179

				161.51		99.15179

				161.54		99.14659

				161.56		99.14659

				161.58		99.14659

				161.6		99.14659

				161.62		99.14139

				161.64		99.14139

				161.66		99.14139

				161.68		99.13618

				161.7		99.13618

				161.72		99.13098

				161.75		99.13098

				161.77		99.12577

				161.79		99.12577

				161.81		99.12577

				161.83		99.12577

				161.85		99.12057

				161.87		99.12057

				161.89		99.12057

				161.91		99.11537

				161.94		99.11537

				161.96		99.11537

				161.98		99.11016

				162		99.11016

				162.02		99.11016

				162.04		99.10496

				162.06		99.10496

				162.08		99.10496

				162.1		99.10496

				162.13		99.10496

				162.15		99.10496

				162.17		99.09976

				162.19		99.09976

				162.21		99.09976

				162.23		99.09455

				162.25		99.09455

				162.27		99.08935

				162.29		99.08935

				162.32		99.08935

				162.34		99.08935

				162.36		99.08414

				162.38		99.08414

				162.4		99.08414

				162.42		99.07894

				162.44		99.07894

				162.46		99.07894

				162.48		99.07374

				162.5		99.07374

				162.53		99.07374

				162.55		99.06853

				162.57		99.06853

				162.59		99.06853

				162.61		99.06333

				162.63		99.06333

				162.65		99.06333

				162.67		99.05813

				162.69		99.05813

				162.72		99.05813

				162.74		99.05813

				162.76		99.05292

				162.78		99.05292

				162.8		99.05292

				162.82		99.04772

				162.84		99.04772

				162.86		99.04251

				162.88		99.04251

				162.91		99.04251

				162.93		99.03731

				162.95		99.03731

				162.97		99.03211

				162.99		99.03211

				163.01		99.03211

				163.03		99.0269

				163.05		99.0269

				163.07		99.0269

				163.1		99.0269

				163.12		99.0269

				163.14		99.0217

				163.16		99.0217

				163.18		99.0165

				163.2		99.0165

				163.22		99.0165

				163.24		99.0165

				163.26		99.01129

				163.29		99.01129

				163.31		99.01129

				163.33		99.01129

				163.35		99.00609

				163.37		99.00609

				163.39		99.00088

				163.41		99.00088

				163.43		99.00088

				163.45		99.00088

				163.48		98.99568

				163.5		98.99568

				163.52		98.99568

				163.54		98.99048

				163.56		98.99048

				163.58		98.99048

				163.6		98.98527

				163.62		98.98527

				163.64		98.98007

				163.67		98.98527

				163.69		98.98007

				163.71		98.98007

				163.73		98.98007

				163.75		98.98007

				163.77		98.98007

				163.79		98.98007

				163.81		98.97487

				163.83		98.97487

				163.86		98.96966

				163.88		98.96966

				163.9		98.96966

				163.92		98.96446

				163.94		98.96446

				163.96		98.96446

				163.98		98.95925

				164		98.95925

				164.02		98.95405

				164.04		98.95405

				164.07		98.95405

				164.09		98.94885

				164.11		98.94364

				164.13		98.94364

				164.15		98.94364

				164.17		98.93844

				164.19		98.93844

				164.21		98.93844

				164.23		98.93844

				164.26		98.93324

				164.28		98.93324

				164.3		98.93324

				164.32		98.93324

				164.34		98.92803

				164.36		98.92803

				164.38		98.92803

				164.4		98.92283

				164.42		98.92283

				164.45		98.91763

				164.47		98.91242

				164.49		98.91242

				164.51		98.90722

				164.53		98.90722

				164.55		98.90201

				164.57		98.90201

				164.59		98.89681

				164.61		98.89681

				164.64		98.89681

				164.66		98.89681

				164.68		98.89681

				164.7		98.89161

				164.72		98.89681

				164.74		98.89161

				164.76		98.89161

				164.78		98.8864

				164.8		98.89161

				164.83		98.8864

				164.85		98.8864

				164.87		98.8812

				164.89		98.8812

				164.91		98.876

				164.93		98.876

				164.95		98.87079

				164.97		98.87079

				164.99		98.87079

				165.01		98.86559

				165.04		98.86038

				165.06		98.85518

				165.08		98.85518

				165.1		98.85518

				165.12		98.84998

				165.14		98.84998

				165.16		98.84998

				165.18		98.84477

				165.2		98.84998

				165.23		98.84998

				165.25		98.84477

				165.27		98.84477

				165.29		98.84477

				165.31		98.84477

				165.33		98.83957

				165.35		98.83957

				165.37		98.83957

				165.39		98.83957

				165.42		98.82916

				165.44		98.82916

				165.46		98.82916

				165.48		98.82916

				165.5		98.82396

				165.52		98.82396

				165.54		98.82396

				165.56		98.81875

				165.58		98.81875

				165.6		98.81875

				165.63		98.81355

				165.65		98.81355

				165.67		98.81355

				165.69		98.81355

				165.71		98.81875

				165.73		98.81355

				165.75		98.81355

				165.77		98.81355

				165.79		98.80835

				165.82		98.80835

				165.84		98.80314

				165.86		98.80314

				165.88		98.79794

				165.9		98.79274

				165.92		98.79274

				165.94		98.78753

				165.96		98.78753

				165.98		98.78233

				166		98.78233

				166.03		98.78233

				166.05		98.77712

				166.07		98.77712

				166.09		98.77712

				166.11		98.77712

				166.13		98.77192

				166.15		98.77192

				166.17		98.77192

				166.19		98.77192

				166.22		98.77192

				166.24		98.76672

				166.26		98.76672

				166.28		98.76151

				166.3		98.75631

				166.32		98.75631

				166.34		98.75111

				166.36		98.7459

				166.38		98.7459

				166.41		98.7459

				166.43		98.73549

				166.45		98.73549

				166.47		98.73549

				166.49		98.73549

				166.51		98.73029

				166.53		98.73549

				166.55		98.73029

				166.57		98.73029

				166.59		98.73029

				166.62		98.72509

				166.64		98.72509

				166.66		98.72509

				166.68		98.72509

				166.7		98.71988

				166.72		98.71468

				166.74		98.71468

				166.76		98.71468

				166.78		98.70948

				166.81		98.70427

				166.83		98.70427

				166.85		98.69907

				166.87		98.69386

				166.89		98.69386

				166.91		98.69386

				166.93		98.68866

				166.95		98.68866

				166.97		98.68866

				167		98.68866

				167.02		98.68346

				167.04		98.68346

				167.06		98.68346

				167.08		98.67825

				167.1		98.67825

				167.12		98.67305

				167.14		98.67305

				167.16		98.66785

				167.18		98.66785

				167.21		98.66264

				167.23		98.65744

				167.25		98.66264

				167.27		98.65744

				167.29		98.65224

				167.31		98.65224

				167.33		98.65224

				167.35		98.64183

				167.37		98.64183

				167.4		98.64183

				167.42		98.64183

				167.44		98.63662

				167.46		98.63662

				167.48		98.63662

				167.5		98.63142

				167.52		98.63142

				167.54		98.62622

				167.56		98.62622

				167.58		98.62101

				167.61		98.62101

				167.63		98.62101

				167.65		98.61581

				167.67		98.61581

				167.69		98.61581

				167.71		98.61581

				167.73		98.61061

				167.75		98.61061

				167.77		98.61061

				167.8		98.61061

				167.82		98.61061

				167.84		98.61061

				167.86		98.6054

				167.88		98.6002

				167.9		98.6002

				167.92		98.59499

				167.94		98.58979

				167.96		98.58979

				167.98		98.58979

				168.01		98.58979

				168.03		98.57938

				168.05		98.58459

				168.07		98.57938

				168.09		98.57938

				168.11		98.57938

				168.13		98.57938

				168.15		98.57418

				168.17		98.57418

				168.19		98.57418

				168.22		98.56898

				168.24		98.56898

				168.26		98.56898

				168.28		98.56377

				168.3		98.55857

				168.32		98.56377

				168.34		98.55857

				168.36		98.55857

				168.38		98.54816

				168.41		98.54816

				168.43		98.54296

				168.45		98.54296

				168.47		98.53255

				168.49		98.53255

				168.51		98.53255

				168.53		98.53255

				168.55		98.52735

				168.57		98.53255

				168.59		98.52735

				168.62		98.52214

				168.64		98.52214

				168.66		98.52214

				168.68		98.51694

				168.7		98.51173

				168.72		98.51173

				168.74		98.51173

				168.76		98.50133

				168.78		98.50653

				168.81		98.50133

				168.83		98.49612

				168.85		98.49092

				168.87		98.48572

				168.89		98.48572

				168.91		98.48051

				168.93		98.48051

				168.95		98.48572

				168.97		98.48051

				168.99		98.47531

				169.02		98.48051

				169.04		98.47531

				169.06		98.4701

				169.08		98.4701

				169.1		98.4701

				169.12		98.4649

				169.14		98.4597

				169.16		98.4597

				169.18		98.4649

				169.21		98.45449

				169.23		98.45449

				169.25		98.45449

				169.27		98.45449

				169.29		98.44929

				169.31		98.45449

				169.33		98.44929

				169.35		98.44409

				169.37		98.44409

				169.39		98.44929

				169.42		98.43888

				169.44		98.43888

				169.46		98.43888

				169.48		98.43368

				169.5		98.42327

				169.52		98.42847

				169.54		98.42327

				169.56		98.41807

				169.58		98.41807

				169.6		98.41807

				169.63		98.41286

				169.65		98.41286

				169.67		98.41286

				169.69		98.40246

				169.71		98.39725

				169.73		98.39725

				169.75		98.40246

				169.77		98.39205

				169.79		98.38684

				169.82		98.39205

				169.84		98.38164

				169.86		98.37644

				169.88		98.37644

				169.9		98.37123

				169.92		98.36603

				169.94		98.36083

				169.96		98.36083

				169.98		98.35562

				170		98.35562

				170.03		98.35562

				170.05		98.35562

				170.07		98.35042

				170.09		98.35042

				170.11		98.35042

				170.13		98.34522

				170.15		98.34001

				170.17		98.34001

				170.19		98.34001

				170.21		98.33481

				170.24		98.33481

				170.26		98.3296

				170.28		98.3296

				170.3		98.3296

				170.32		98.3296

				170.34		98.3192

				170.36		98.3192

				170.38		98.31399

				170.4		98.3192

				170.43		98.31399

				170.45		98.30879

				170.47		98.30879

				170.49		98.30359

				170.51		98.30359

				170.53		98.30359

				170.55		98.29838

				170.57		98.29318

				170.59		98.29318

				170.61		98.29838

				170.64		98.28797

				170.66		98.28797

				170.68		98.29318

				170.7		98.28797

				170.72		98.28277

				170.74		98.28277

				170.76		98.28277

				170.78		98.27236

				170.8		98.27236

				170.82		98.26716

				170.85		98.26196

				170.87		98.25675

				170.89		98.26196

				170.91		98.26196

				170.93		98.25155

				170.95		98.25675

				170.97		98.25675

				170.99		98.25155

				171.01		98.24634

				171.03		98.24634

				171.06		98.24114

				171.08		98.24114

				171.1		98.23594

				171.12		98.23594

				171.14		98.22553

				171.16		98.22553

				171.18		98.22553

				171.2		98.21512

				171.22		98.21512

				171.24		98.21512

				171.26		98.20992

				171.29		98.20471

				171.31		98.20471

				171.33		98.20471

				171.35		98.20471

				171.37		98.19951

				171.39		98.19951

				171.41		98.19431

				171.43		98.1891

				171.45		98.19431

				171.47		98.1891

				171.5		98.1839

				171.52		98.1839

				171.54		98.1839

				171.56		98.1839

				171.58		98.1787

				171.6		98.1787

				171.62		98.17349

				171.64		98.16829

				171.66		98.16829

				171.68		98.16829

				171.71		98.16308

				171.73		98.16308

				171.75		98.16308

				171.77		98.15268

				171.79		98.14747

				171.81		98.14747

				171.83		98.14747

				171.85		98.14227

				171.87		98.13707

				171.89		98.13707

				171.92		98.13707

				171.94		98.13186

				171.96		98.13707

				171.98		98.12666

				172		98.12666

				172.02		98.12666

				172.04		98.12666

				172.06		98.12145

				172.08		98.12145

				172.1		98.12145

				172.13		98.11625

				172.15		98.12145

				172.17		98.11625

				172.19		98.11105

				172.21		98.11625

				172.23		98.11105

				172.25		98.10584

				172.27		98.10064

				172.29		98.10584

				172.31		98.10064

				172.34		98.09544

				172.36		98.09023

				172.38		98.09023

				172.4		98.08503

				172.42		98.08503

				172.44		98.08503

				172.46		98.07983

				172.48		98.07462

				172.5		98.06942

				172.52		98.06942

				172.55		98.06942

				172.57		98.06421

				172.59		98.05901

				172.61		98.0486

				172.63		98.0434

				172.65		98.0434

				172.67		98.0382

				172.69		98.03299

				172.71		98.03299

				172.73		98.02258

				172.76		98.02258

				172.78		98.02258

				172.8		98.02258

				172.82		98.02258

				172.84		98.01218

				172.86		98.01218

				172.88		98.00697

				172.9		98.00177

				172.92		98.00177

				172.94		97.99136

				172.97		97.99657

				172.99		97.99136

				173.01		97.98616

				173.03		97.98616

				173.05		97.98095

				173.07		97.98095

				173.09		97.98095

				173.11		97.97575

				173.13		97.97575

				173.15		97.97055

				173.18		97.97575

				173.2		97.97055

				173.22		97.97055

				173.24		97.97055

				173.26		97.97055

				173.28		97.96534

				173.3		97.96014

				173.32		97.96014

				173.34		97.96014

				173.36		97.95494

				173.39		97.95494

				173.41		97.95494

				173.43		97.94973

				173.45		97.95494

				173.47		97.94973

				173.49		97.94453

				173.51		97.93932

				173.53		97.94453

				173.55		97.93932

				173.57		97.93412

				173.59		97.92892

				173.62		97.92892

				173.64		97.92892

				173.66		97.92371

				173.68		97.92371

				173.7		97.91851

				173.72		97.91331

				173.74		97.91331

				173.76		97.9081

				173.78		97.9029

				173.8		97.9029

				173.83		97.9029

				173.85		97.89769

				173.87		97.89249

				173.89		97.89249

				173.91		97.89249

				173.93		97.88729

				173.95		97.88729

				173.97		97.88208

				173.99		97.87688

				174.01		97.87688

				174.04		97.87688

				174.06		97.87168

				174.08		97.87168

				174.1		97.86647

				174.12		97.86647

				174.14		97.86647

				174.16		97.86127

				174.18		97.86127

				174.2		97.85606

				174.22		97.85606

				174.25		97.85086

				174.27		97.85086

				174.29		97.85086

				174.31		97.85086

				174.33		97.84566

				174.35		97.84566

				174.37		97.84045

				174.39		97.83525

				174.41		97.83525

				174.43		97.83005

				174.46		97.83005

				174.48		97.83005

				174.5		97.82484

				174.52		97.82484

				174.54		97.82484

				174.56		97.81964

				174.58		97.81964

				174.6		97.80923

				174.62		97.80923

				174.64		97.79882

				174.67		97.79882

				174.69		97.79362

				174.71		97.79362

				174.73		97.78321

				174.75		97.78321

				174.77		97.78321

				174.79		97.78321

				174.81		97.77281

				174.83		97.77281

				174.85		97.77801

				174.88		97.77281

				174.9		97.77281

				174.92		97.7676

				174.94		97.7624

				174.96		97.75719

				174.98		97.75199

				175		97.75199

				175.02		97.74679

				175.04		97.74679

				175.06		97.74158

				175.09		97.73638

				175.11		97.73638

				175.13		97.72597

				175.15		97.73118

				175.17		97.72597

				175.19		97.72077

				175.21		97.71556

				175.23		97.71556

				175.25		97.70516

				175.27		97.70516

				175.29		97.69995

				175.32		97.69475

				175.34		97.69475

				175.36		97.68955

				175.38		97.68955

				175.4		97.68434

				175.42		97.68434

				175.44		97.68434

				175.46		97.67914

				175.48		97.67393

				175.5		97.66873

				175.53		97.66873

				175.55		97.66353

				175.57		97.66353

				175.59		97.65832

				175.61		97.65312

				175.63		97.65312

				175.65		97.64792

				175.67		97.64271

				175.69		97.63751

				175.71		97.6323

				175.74		97.6271

				175.76		97.6271

				175.78		97.6219

				175.8		97.6219

				175.82		97.61669

				175.84		97.61149

				175.86		97.61149

				175.88		97.60629

				175.9		97.60629

				175.92		97.60629

				175.95		97.60629

				175.97		97.60108

				175.99		97.59588

				176.01		97.59067

				176.03		97.59067

				176.05		97.59067

				176.07		97.58027

				176.09		97.58547

				176.11		97.57506

				176.13		97.57506

				176.15		97.56986

				176.18		97.56466

				176.2		97.55945

				176.22		97.56466

				176.24		97.55425

				176.26		97.55425

				176.28		97.55425

				176.3		97.54905

				176.32		97.54905

				176.34		97.54384

				176.36		97.54384

				176.39		97.53864

				176.41		97.53864

				176.43		97.53343

				176.45		97.52823

				176.47		97.52303

				176.49		97.52303

				176.51		97.52303

				176.53		97.51262

				176.55		97.51782

				176.57		97.51262

				176.6		97.50742

				176.62		97.50221

				176.64		97.49701

				176.66		97.4918

				176.68		97.4866

				176.7		97.4814

				176.72		97.4814

				176.74		97.47619

				176.76		97.47099

				176.78		97.47099

				176.81		97.47099

				176.83		97.46058

				176.85		97.46579

				176.87		97.46058

				176.89		97.45538

				176.91		97.45017

				176.93		97.45538

				176.95		97.44497

				176.97		97.44497

				176.99		97.44497

				177.01		97.43977

				177.04		97.43456

				177.06		97.43456

				177.08		97.42936

				177.1		97.42416

				177.12		97.41895

				177.14		97.42416

				177.16		97.41895

				177.18		97.41375

				177.2		97.40334

				177.22		97.40334

				177.25		97.39814

				177.27		97.39814

				177.29		97.39293

				177.31		97.39293

				177.33		97.38773

				177.35		97.39293

				177.37		97.38773

				177.39		97.38253

				177.41		97.38253

				177.43		97.38253

				177.46		97.37732

				177.48		97.37212

				177.5		97.37212

				177.52		97.36691

				177.54		97.35651

				177.56		97.35651

				177.58		97.35651

				177.6		97.3513

				177.62		97.3461

				177.64		97.3461

				177.66		97.33569

				177.69		97.33569

				177.71		97.33049

				177.73		97.33049

				177.75		97.32008

				177.77		97.32008

				177.79		97.30967

				177.81		97.31488

				177.83		97.30967

				177.85		97.30967

				177.87		97.30967

				177.9		97.30447

				177.92		97.30447

				177.94		97.30447

				177.96		97.29406

				177.98		97.29406

				178		97.29406

				178.02		97.29406

				178.04		97.28366

				178.06		97.28366

				178.08		97.27845

				178.11		97.27845

				178.13		97.27325

				178.15		97.27325

				178.17		97.26804

				178.19		97.26284

				178.21		97.25764

				178.23		97.25764

				178.25		97.24723

				178.27		97.25243

				178.29		97.24723

				178.31		97.24203

				178.34		97.24203

				178.36		97.23682

				178.38		97.23162

				178.4		97.23162

				178.42		97.23162

				178.44		97.22121

				178.46		97.22121

				178.48		97.2108

				178.5		97.2056

				178.52		97.2056

				178.55		97.2004

				178.57		97.19519

				178.59		97.18999

				178.61		97.18999

				178.63		97.18999

				178.65		97.18999

				178.67		97.17958

				178.69		97.17438

				178.71		97.16917

				178.73		97.16917

				178.75		97.16917

				178.78		97.15877

				178.8		97.15877

				178.82		97.15877

				178.84		97.15877

				178.86		97.15877

				178.88		97.15356

				178.9		97.14836

				178.92		97.14836

				178.94		97.13795

				178.96		97.14315

				178.99		97.13275

				179.01		97.13275

				179.03		97.12234

				179.05		97.11714

				179.07		97.11714

				179.09		97.11193

				179.11		97.10673

				179.13		97.10152

				179.15		97.09632

				179.17		97.09112

				179.19		97.09112

				179.22		97.08591

				179.24		97.08591

				179.26		97.08071

				179.28		97.08071

				179.3		97.08071

				179.32		97.0703

				179.34		97.08071

				179.36		97.0703

				179.38		97.07551

				179.4		97.07551

				179.42		97.0703

				179.45		97.0651

				179.47		97.0651

				179.49		97.05989

				179.51		97.05989

				179.53		97.05469

				179.55		97.04949

				179.57		97.04428

				179.59		97.03388

				179.61		97.02867

				179.63		97.02347

				179.65		97.01827

				179.68		97.00786

				179.7		97.00786

				179.72		96.99745

				179.74		96.99225

				179.76		96.99745

				179.78		96.99225

				179.8		96.98184

				179.82		96.98704

				179.84		96.98184

				179.86		96.97664

				179.89		96.97664

				179.91		96.98184

				179.93		96.98184

				179.95		96.97664

				179.97		96.97143

				179.99		96.97664

				180.01		96.96623

				180.03		96.95582

				180.05		96.95582

				180.07		96.95062

				180.09		96.93501

				180.12		96.94021

				180.14		96.93501

				180.16		96.9246

				180.18		96.91939

				180.2		96.91939

				180.22		96.90899

				180.24		96.90378

				180.26		96.89858

				180.28		96.90378

				180.3		96.88817

				180.33		96.88817

				180.35		96.89858

				180.37		96.88297

				180.39		96.87776

				180.41		96.89338

				180.43		96.87776

				180.45		96.87256

				180.47		96.86736

				180.49		96.87256

				180.51		96.85175

				180.53		96.85175

				180.56		96.85175

				180.58		96.84654

				180.6		96.83093

				180.62		96.83093

				180.64		96.82573

				180.66		96.81012

				180.68		96.81532

				180.7		96.82052

				180.72		96.79971

				180.74		96.7945

				180.77		96.7945

				180.79		96.7945

				180.81		96.77889

				180.83		96.7893

				180.85		96.7841

				180.87		96.77369

				180.89		96.76849

				180.91		96.77369

				180.93		96.76849

				180.95		96.76328

				180.97		96.76328

				181		96.76328

				181.02		96.74767

				181.04		96.74767

				181.06		96.74767

				181.08		96.73726

				181.1		96.72686

				181.12		96.73206

				181.14		96.72686

				181.16		96.71645

				181.18		96.71645

				181.21		96.72165

				181.23		96.70084

				181.25		96.70084

				181.27		96.70084

				181.29		96.69563

				181.31		96.68523

				181.33		96.68523

				181.35		96.68523

				181.37		96.68002

				181.39		96.68002

				181.41		96.68002

				181.44		96.67482

				181.46		96.66962

				181.48		96.66962

				181.5		96.66962

				181.52		96.654

				181.54		96.65921

				181.56		96.65921

				181.58		96.6488

				181.6		96.6436

				181.62		96.6436

				181.64		96.63319

				181.67		96.62799

				181.69		96.61758

				181.71		96.61758

				181.73		96.60197

				181.75		96.59676

				181.77		96.60197

				181.79		96.59676

				181.81		96.58636

				181.83		96.59156

				181.85		96.59676

				181.88		96.58115

				181.9		96.58115

				181.92		96.58115

				181.94		96.58115

				181.96		96.57595

				181.98		96.57595

				182		96.58115

				182.02		96.57074

				182.04		96.58115

				182.06		96.57074

				182.08		96.56034

				182.11		96.55513

				182.13		96.56034

				182.15		96.54993

				182.17		96.53432

				182.19		96.52911

				182.21		96.52911

				182.23		96.52391

				182.25		96.5135

				182.27		96.5135

				182.29		96.5083

				182.31		96.49789

				182.34		96.5031

				182.36		96.49269

				182.38		96.48749

				182.4		96.48749

				182.42		96.48228

				182.44		96.47187

				182.46		96.47708

				182.48		96.47708

				182.5		96.47708

				182.52		96.46667

				182.55		96.46147

				182.57		96.45626

				182.59		96.45106

				182.61		96.44586

				182.63		96.44586

				182.65		96.43545

				182.67		96.43024

				182.69		96.43024

				182.71		96.42504

				182.73		96.40943

				182.75		96.40943

				182.78		96.40943

				182.8		96.40423

				182.82		96.39902

				182.84		96.39902

				182.86		96.39902

				182.88		96.39382

				182.9		96.38861

				182.92		96.38861

				182.94		96.37821

				182.96		96.38341

				182.99		96.373

				183.01		96.373

				183.03		96.37821

				183.05		96.3626

				183.07		96.35739

				183.09		96.35219

				183.11		96.35219

				183.13		96.34698

				183.15		96.34178

				183.17		96.33137

				183.19		96.33137

				183.22		96.32097

				183.24		96.32097

				183.26		96.32097

				183.28		96.31056

				183.3		96.31576

				183.32		96.31576

				183.34		96.30535

				183.36		96.30015

				183.38		96.30535

				183.4		96.30015

				183.43		96.28454

				183.45		96.28974

				183.47		96.28454

				183.49		96.28454

				183.51		96.27934

				183.53		96.26372

				183.55		96.26893

				183.57		96.25852

				183.59		96.24811

				183.61		96.24811

				183.63		96.24291

				183.66		96.2325

				183.68		96.21689

				183.7		96.21169

				183.72		96.20648

				183.74		96.19608

				183.76		96.19608

				183.78		96.19087

				183.8		96.18567

				183.82		96.17526

				183.84		96.17006

				183.87		96.17006

				183.89		96.16485

				183.91		96.15965

				183.93		96.15965

				183.95		96.15965

				183.97		96.15965

				183.99		96.15445

				184.01		96.15445

				184.03		96.14924

				184.05		96.13884

				184.07		96.13363

				184.1		96.12843

				184.12		96.11802

				184.14		96.11802

				184.16		96.11282

				184.18		96.10761

				184.2		96.092

				184.22		96.092

				184.24		96.092

				184.26		96.08159

				184.28		96.07639

				184.3		96.08159

				184.33		96.08159

				184.35		96.07639

				184.37		96.07119

				184.39		96.08159

				184.41		96.07639

				184.43		96.07639

				184.45		96.07639

				184.47		96.07639

				184.49		96.06598

				184.51		96.06078

				184.53		96.07119

				184.56		96.05558

				184.58		96.05037

				184.6		96.03996

				184.62		96.03476

				184.64		96.02435

				184.66		96.01395

				184.68		96.00874

				184.7		95.99313

				184.72		95.99313

				184.74		95.98793

				184.76		95.98272

				184.79		95.97232

				184.81		95.96711

				184.83		95.96711

				184.85		95.95671

				184.87		95.96191

				184.89		95.96191

				184.91		95.95671

				184.93		95.9515

				184.95		95.9463

				184.97		95.95671

				185		95.9463

				185.02		95.94109

				185.04		95.94109

				185.06		95.93589

				185.08		95.93069

				185.1		95.92548

				185.12		95.92548

				185.14		95.91508

				185.16		95.90987

				185.18		95.90467

				185.2		95.89946

				185.23		95.89426

				185.25		95.88385

				185.27		95.88385

				185.29		95.87345

				185.31		95.86824

				185.33		95.85783

				185.35		95.85783

				185.37		95.84743

				185.39		95.84222

				185.41		95.83702

				185.44		95.82661

				185.46		95.8162

				185.48		95.82141

				185.5		95.8162

				185.52		95.8162

				185.54		95.8162

				185.56		95.811

				185.58		95.80059

				185.6		95.80059

				185.62		95.79019

				185.64		95.79019

				185.67		95.77978

				185.69		95.77978

				185.71		95.76937

				185.73		95.76417

				185.75		95.75376

				185.77		95.74856

				185.79		95.73294

				185.81		95.73294

				185.83		95.72774

				185.85		95.72254

				185.87		95.71213

				185.9		95.71213

				185.92		95.70693

				185.94		95.70172

				185.96		95.70172

				185.98		95.70693

				186		95.69652

				186.02		95.69652

				186.04		95.69131

				186.06		95.69652

				186.08		95.68611

				186.1		95.68091

				186.13		95.68611

				186.15		95.6757

				186.17		95.6653

				186.19		95.66009

				186.21		95.6653

				186.23		95.64448

				186.25		95.63928

				186.27		95.62887

				186.29		95.62367

				186.31		95.61326

				186.33		95.61326

				186.36		95.60285

				186.38		95.59765

				186.4		95.59244

				186.42		95.59244

				186.44		95.57683

				186.46		95.58204

				186.48		95.57163

				186.5		95.57683

				186.52		95.57163

				186.54		95.57683

				186.56		95.56643

				186.59		95.57163

				186.61		95.56122

				186.63		95.56122

				186.65		95.55081

				186.67		95.54561

				186.69		95.5352

				186.71		95.54041

				186.73		95.51959

				186.75		95.5248

				186.77		95.51439

				186.79		95.50918

				186.82		95.49357

				186.84		95.49357

				186.86		95.48837

				186.88		95.48317

				186.9		95.47796

				186.92		95.46755

				186.94		95.45194

				186.96		95.45194

				186.98		95.44674

				187		95.43113

				187.02		95.43113

				187.05		95.42592

				187.07		95.42592

				187.09		95.41552

				187.11		95.41031

				187.13		95.40511

				187.15		95.39991

				187.17		95.40511

				187.19		95.40511

				187.21		95.3843

				187.23		95.3895

				187.25		95.3895

				187.28		95.3843

				187.3		95.37909

				187.32		95.37389

				187.34		95.36868

				187.36		95.35828

				187.38		95.35828

				187.4		95.33746

				187.42		95.33746

				187.44		95.33226

				187.46		95.32705

				187.48		95.32185

				187.51		95.31665

				187.53		95.30624

				187.55		95.30624

				187.57		95.30624

				187.59		95.29583

				187.61		95.29063

				187.63		95.28542

				187.65		95.28022

				187.67		95.26461

				187.69		95.25941

				187.71		95.2542

				187.74		95.249

				187.76		95.23859

				187.78		95.23339

				187.8		95.22818

				187.82		95.22818

				187.84		95.22298

				187.86		95.22298

				187.88		95.21257

				187.9		95.21778

				187.92		95.21257

				187.94		95.19696

				187.97		95.19176

				187.99		95.18655

				188.01		95.18655

				188.03		95.17615

				188.05		95.17094

				188.07		95.16053

				188.09		95.16053

				188.11		95.15533

				188.13		95.15013

				188.15		95.14492

				188.18		95.13452

				188.2		95.12931

				188.22		95.12931

				188.24		95.11891

				188.26		95.1137

				188.28		95.1085

				188.3		95.10329

				188.32		95.09289

				188.34		95.08768

				188.36		95.08248

				188.38		95.08248

				188.41		95.08248

				188.43		95.07207

				188.45		95.06687

				188.47		95.06166

				188.49		95.05646

				188.51		95.04605

				188.53		95.04085

				188.55		95.03565

				188.57		95.02524

				188.59		95.02003

				188.61		95.00963

				188.64		95.00963

				188.66		95.00442

				188.68		94.99922

				188.7		94.99402

				188.72		94.98881

				188.74		94.98361

				188.76		94.98361

				188.78		94.9732

				188.8		94.9732

				188.82		94.95239

				188.84		94.95239

				188.87		94.94198

				188.89		94.93157

				188.91		94.93157

				188.93		94.93157

				188.95		94.92116

				188.97		94.92116

				188.99		94.90555

				189.01		94.90555

				189.03		94.90035

				189.05		94.90035

				189.07		94.89514

				189.1		94.88474

				189.12		94.88474

				189.14		94.87953

				189.16		94.86392

				189.18		94.85872

				189.2		94.84831

				189.22		94.85352

				189.24		94.84311

				189.26		94.8327

				189.28		94.8327

				189.3		94.82229

				189.33		94.81709

				189.35		94.81189

				189.37		94.80148

				189.39		94.80148

				189.41		94.79107

				189.43		94.79627

				189.45		94.78066

				189.47		94.77546

				189.49		94.77546

				189.51		94.77026

				189.53		94.75985

				189.56		94.75464

				189.58		94.73903

				189.6		94.73383

				189.62		94.72863

				189.64		94.71822

				189.66		94.70781

				189.68		94.70261

				189.7		94.6974

				189.72		94.6922

				189.74		94.68179

				189.76		94.67659

				189.79		94.67659

				189.81		94.67138

				189.83		94.66618

				189.85		94.65577

				189.87		94.66098

				189.89		94.64537

				189.91		94.64537

				189.93		94.64016

				189.95		94.62975

				189.97		94.61935

				189.99		94.61935

				190.02		94.61935

				190.04		94.61414

				190.06		94.61414

				190.08		94.60374

				190.1		94.59853

				190.12		94.58813

				190.14		94.58813

				190.16		94.58813

				190.18		94.58813

				190.2		94.56731

				190.22		94.56211

				190.25		94.5465

				190.27		94.5465

				190.29		94.5465

				190.31		94.54129

				190.33		94.52048

				190.35		94.51527

				190.37		94.50487

				190.39		94.50487

				190.41		94.48925

				190.43		94.48405

				190.45		94.47364

				190.48		94.46324

				190.5		94.45283

				190.52		94.45803

				190.54		94.44762

				190.56		94.44242

				190.58		94.44762

				190.6		94.44762

				190.62		94.43722

				190.64		94.43722

				190.66		94.42161

				190.68		94.42681

				190.71		94.4112

				190.73		94.40599

				190.75		94.40079

				190.77		94.38518

				190.79		94.37998

				190.81		94.37998

				190.83		94.36436

				190.85		94.36957

				190.87		94.35396

				190.89		94.35916

				190.91		94.33835

				190.94		94.33835

				190.96		94.33835

				190.98		94.32274

				191		94.30712

				191.02		94.31233

				191.04		94.30712

				191.06		94.29672

				191.08		94.29672

				191.1		94.29672

				191.12		94.28111

				191.14		94.2707

				191.17		94.25509

				191.19		94.26549

				191.21		94.24468

				191.23		94.23427

				191.25		94.22386

				191.27		94.21346

				191.29		94.20305

				191.31		94.19785

				191.33		94.19264

				191.35		94.20305

				191.37		94.18744

				191.4		94.18223

				191.42		94.17703

				191.44		94.16662

				191.46		94.16662

				191.48		94.16142

				191.5		94.15622

				191.52		94.14581

				191.54		94.1302

				191.56		94.12499

				191.58		94.12499

				191.6		94.12499

				191.63		94.11459

				191.65		94.09897

				191.67		94.08857

				191.69		94.08857

				191.71		94.06775

				191.73		94.07296

				191.75		94.06255

				191.77		94.05214

				191.79		94.03653

				191.81		94.04694

				191.83		94.03133

				191.85		94.03653

				191.88		94.02092

				191.9		94.02092

				191.92		94.01572

				191.94		94.00531

				191.96		94.0001

				191.98		93.9897

				192		93.98449

				192.02		93.97929

				192.04		93.97409

				192.06		93.96888

				192.08		93.96368

				192.11		93.95847

				192.13		93.95847

				192.15		93.94807

				192.17		93.95327

				192.19		93.93766

				192.21		93.93766

				192.23		93.92725

				192.25		93.92205

				192.27		93.91164

				192.29		93.90123

				192.31		93.89603

				192.34		93.88562

				192.36		93.87521

				192.38		93.87001

				192.4		93.87001

				192.42		93.8492

				192.44		93.8492

				192.46		93.84399

				192.48		93.83879

				192.5		93.81797

				192.52		93.82318

				192.54		93.81277

				192.57		93.80757

				192.59		93.80236

				192.61		93.79196

				192.63		93.78675

				192.65		93.77634

				192.67		93.77114

				192.69		93.77114

				192.71		93.75553

				192.73		93.74512

				192.75		93.74512

				192.77		93.72431

				192.8		93.72951

				192.82		93.7191

				192.84		93.7087

				192.86		93.69308

				192.88		93.69308

				192.9		93.68268

				192.92		93.68268

				192.94		93.67227

				192.96		93.67747

				192.98		93.66707

				193		93.65666

				193.03		93.66186

				193.05		93.66186

				193.07		93.64625

				193.09		93.63584

				193.11		93.63064

				193.13		93.60982

				193.15		93.60462

				193.17		93.59421

				193.19		93.58901

				193.21		93.5734

				193.23		93.56299

				193.26		93.56299

				193.28		93.55258

				193.3		93.54218

				193.32		93.54218

				193.34		93.52657

				193.36		93.52136

				193.38		93.51095

				193.4		93.50575

				193.42		93.50055

				193.44		93.48494

				193.46		93.50055

				193.49		93.47973

				193.51		93.47453

				193.53		93.47453

				193.55		93.47973

				193.57		93.47453

				193.59		93.46932

				193.61		93.46412

				193.63		93.45892

				193.65		93.4381

				193.67		93.4381

				193.69		93.4329

				193.72		93.41208

				193.74		93.40168

				193.76		93.39127

				193.78		93.37045

				193.8		93.36005

				193.82		93.34964

				193.84		93.34964

				193.86		93.32882

				193.88		93.31842

				193.9		93.31321

				193.92		93.3028

				193.95		93.31321

				193.97		93.3028

				193.99		93.28719

				194.01		93.28199

				194.03		93.28199

				194.05		93.27679

				194.07		93.27158

				194.09		93.27158

				194.11		93.26638

				194.13		93.25597

				194.15		93.25077

				194.18		93.25077

				194.2		93.22995

				194.22		93.22475

				194.24		93.21955

				194.26		93.20914

				194.28		93.20914

				194.3		93.17271

				194.32		93.18312

				194.34		93.17271

				194.36		93.16751

				194.38		93.1571

				194.41		93.14149

				194.43		93.13629

				194.45		93.13108

				194.47		93.11547

				194.49		93.10506

				194.51		93.11027

				194.53		93.10506

				194.55		93.10506

				194.57		93.09466

				194.59		93.09466

				194.61		93.08425

				194.63		93.08425

				194.66		93.07384

				194.68		93.06343

				194.7		93.05303

				194.72		93.03221

				194.74		93.02701

				194.76		93.0166

				194.78		93.00099

				194.8		92.98538

				194.82		92.97497

				194.84		92.96456

				194.86		92.96456

				194.89		92.94895

				194.91		92.95416

				194.93		92.94895

				194.95		92.94375

				194.97		92.92814

				194.99		92.93334

				195.01		92.92293

				195.03		92.92814

				195.05		92.90212

				195.07		92.89691

				195.09		92.89171

				195.12		92.90212

				195.14		92.8761

				195.16		92.8709

				195.18		92.8709

				195.2		92.85528

				195.22		92.85528

				195.24		92.83447

				195.26		92.82406

				195.28		92.80845

				195.3		92.80325

				195.32		92.78243

				195.35		92.78764

				195.37		92.77202

				195.39		92.78243

				195.41		92.76682

				195.43		92.77202

				195.45		92.76162

				195.47		92.76162

				195.49		92.75641

				195.51		92.74601

				195.53		92.74601

				195.55		92.73039

				195.58		92.71999

				195.6		92.70438

				195.62		92.70438

				195.64		92.68356

				195.66		92.66795

				195.68		92.65754

				195.7		92.65234

				195.72		92.63152

				195.74		92.63152

				195.76		92.61071

				195.78		92.6003

				195.81		92.5951

				195.83		92.58469

				195.85		92.57949

				195.87		92.56388

				195.89		92.56388

				195.91		92.54826

				195.93		92.54306

				195.95		92.53265

				195.97		92.53786

				195.99		92.52745

				196.01		92.53786

				196.04		92.52745

				196.06		92.53265

				196.08		92.53265

				196.1		92.52745

				196.12		92.51184

				196.14		92.50663

				196.16		92.48062

				196.18		92.47021

				196.2		92.47021

				196.22		92.44419

				196.24		92.43378

				196.27		92.42858

				196.29		92.39215

				196.31		92.39215

				196.33		92.38175

				196.35		92.36613

				196.37		92.35573

				196.39		92.35052

				196.41		92.34532

				196.43		92.35052

				196.45		92.35052

				196.47		92.34012

				196.49		92.33491

				196.52		92.3193

				196.54		92.34012

				196.56		92.3141

				196.58		92.3193

				196.6		92.30889

				196.62		92.30889

				196.64		92.27767

				196.66		92.28808

				196.68		92.25165

				196.7		92.25165

				196.72		92.24124

				196.75		92.22043

				196.77		92.21002

				196.79		92.21523

				196.81		92.18921

				196.83		92.19441

				196.85		92.184

				196.87		92.15278

				196.89		92.16319

				196.91		92.15278

				196.93		92.14758

				196.95		92.13197

				196.98		92.12676

				197		92.11115

				197.02		92.11636

				197.04		92.10595

				197.06		92.10074

				197.08		92.09034

				197.1		92.09554

				197.12		92.07993

				197.14		92.07993

				197.16		92.06432

				197.18		92.05391

				197.21		92.04871

				197.23		92.02269

				197.25		92.02789

				197.27		92.00708

				197.29		92.00708

				197.31		91.99147

				197.33		91.98106

				197.35		91.96024

				197.37		91.97065

				197.39		91.94984

				197.41		91.94984

				197.44		91.92902

				197.46		91.93422

				197.48		91.91861

				197.5		91.91341

				197.52		91.8978

				197.54		91.88739

				197.56		91.88739

				197.58		91.86658

				197.6		91.85617

				197.62		91.86137

				197.64		91.86137

				197.66		91.84576

				197.69		91.85097

				197.71		91.84056

				197.73		91.84056

				197.75		91.83015

				197.77		91.82495

				197.79		91.80934

				197.81		91.80413

				197.83		91.78852

				197.85		91.76771

				197.87		91.7625

				197.89		91.74689

				197.92		91.73648

				197.94		91.72087

				197.96		91.71046

				197.98		91.70526

				198		91.70006

				198.02		91.68445

				198.04		91.70006

				198.06		91.69485

				198.08		91.67924

				198.1		91.66883

				198.12		91.67404

				198.15		91.65322

				198.17		91.64282

				198.19		91.6168

				198.21		91.622

				198.23		91.6168

				198.25		91.61159

				198.27		91.59598

				198.29		91.59598

				198.31		91.59078

				198.33		91.58558

				198.35		91.56476

				198.37		91.54915

				198.4		91.54915

				198.42		91.53354

				198.44		91.52313

				198.46		91.49711

				198.48		91.50232

				198.5		91.4815

				198.52		91.4867

				198.54		91.4763

				198.56		91.4815

				198.58		91.47109

				198.6		91.4763

				198.63		91.45028

				198.65		91.45548

				198.67		91.42946

				198.69		91.41385

				198.71		91.40344

				198.73		91.38263

				198.75		91.37743

				198.77		91.37222

				198.79		91.37743

				198.81		91.36702

				198.83		91.36702

				198.86		91.3462

				198.88		91.35141

				198.9		91.3358

				198.92		91.3358

				198.94		91.29937

				198.96		91.30457

				198.98		91.28376

				199		91.27856

				199.02		91.26294

				199.04		91.24733

				199.06		91.24213

				199.08		91.23172

				199.11		91.22131

				199.13		91.22131

				199.15		91.2057

				199.17		91.1953

				199.19		91.1953

				199.21		91.15887

				199.23		91.16407

				199.25		91.12765

				199.27		91.11724

				199.29		91.10163

				199.31		91.09122

				199.33		91.06

				199.36		91.07561

				199.38		91.04439

				199.4		91.0652

				199.42		91.06

				199.44		91.04959

				199.46		91.04959

				199.48		91.04439

				199.5		91.03918

				199.52		91.03398

				199.54		91.03398

				199.56		91.00276

				199.59		90.99235

				199.61		90.97674

				199.63		90.97154

				199.65		90.95592

				199.67		90.95072

				199.69		90.9195

				199.71		90.94031

				199.73		90.9247

				199.75		90.9195

				199.77		90.91429

				199.79		90.89348

				199.82		90.88307

				199.84		90.87266

				199.86		90.85705

				199.88		90.83624

				199.9		90.83624

				199.92		90.82063

				199.94		90.82063

				199.96		90.79981

				199.98		90.79981

				200		90.7842

				200.02		90.78941

				200.04		90.76859

				200.07		90.75818

				200.09		90.74257

				200.11		90.74257

				200.13		90.73737

				200.15		90.72696

				200.17		90.71135

				200.19		90.70615

				200.21		90.70094

				200.23		90.68533

				200.25		90.68013

				200.27		90.65931

				200.3		90.65931

				200.32		90.6437

				200.34		90.63329

				200.36		90.60727

				200.38		90.61248

				200.4		90.59687

				200.42		90.58646

				200.44		90.57085

				200.46		90.56565

				200.48		90.56044

				200.5		90.55524

				200.53		90.54483

				200.55		90.53442

				200.57		90.52922

				200.59		90.51361

				200.61		90.5084

				200.63		90.49279

				200.65		90.48759

				200.67		90.46677

				200.69		90.46157

				200.71		90.43035

				200.73		90.44596

				200.75		90.42514

				200.78		90.42514

				200.8		90.40953

				200.82		90.39913

				200.84		90.38872

				200.86		90.39392

				200.88		90.3627

				200.9		90.3627

				200.92		90.35229

				200.94		90.35229

				200.96		90.35229

				200.98		90.33668

				201.01		90.33668

				201.03		90.32627

				201.05		90.33148

				201.07		90.31066

				201.09		90.30025

				201.11		90.28985

				201.13		90.27944

				201.15		90.25863

				201.17		90.23261

				201.19		90.23261

				201.21		90.2222

				201.23		90.20138

				201.26		90.20138

				201.28		90.19098

				201.3		90.17537

				201.32		90.14935

				201.34		90.14935

				201.36		90.12333

				201.38		90.11812

				201.4		90.10772

				201.42		90.11812

				201.44		90.09211

				201.46		90.09731

				201.49		90.07649

				201.51		90.07129

				201.53		90.04527

				201.55		90.05048

				201.57		90.02966

				201.59		90.04007

				201.61		90.01405

				201.63		90.01925

				201.65		90.00364

				201.67		89.99324

				201.69		89.97242

				201.71		89.97762

				201.74		89.9464

				201.76		89.95161

				201.78		89.93599

				201.8		89.92559

				201.82		89.91518

				201.84		89.92038

				201.86		89.89436

				201.88		89.89957

				201.9		89.91518

				201.92		89.88396

				201.94		89.87875

				201.97		89.86314

				201.99		89.85794

				202.01		89.83192

				202.03		89.82672

				202.05		89.8059

				202.07		89.79029

				202.09		89.76947

				202.11		89.74346

				202.13		89.73825

				202.15		89.71223

				202.17		89.70703

				202.19		89.69662

				202.22		89.70183

				202.24		89.68101

				202.26		89.68622

				202.28		89.68101

				202.3		89.6654

				202.32		89.65499

				202.34		89.64459

				202.36		89.63418

				202.38		89.61336

				202.4		89.60816

				202.42		89.59255

				202.44		89.59775

				202.47		89.58214

				202.49		89.57694

				202.51		89.54571

				202.53		89.53531

				202.55		89.5249

				202.57		89.5197

				202.59		89.51449

				202.61		89.50929

				202.63		89.49888

				202.65		89.48327

				202.67		89.46766

				202.7		89.43644

				202.72		89.44164

				202.74		89.43644

				202.76		89.42603

				202.78		89.43123

				202.8		89.43644

				202.82		89.40521

				202.84		89.40001

				202.86		89.37399

				202.88		89.34797

				202.9		89.32195

				202.92		89.32195

				202.95		89.30114

				202.97		89.30634

				202.99		89.28553

				203.01		89.28032

				203.03		89.27512

				203.05		89.25951

				203.07		89.2439

				203.09		89.2439

				203.11		89.2439

				203.13		89.22829

				203.15		89.21788

				203.17		89.22308

				203.2		89.25431

				203.22		89.22829

				203.24		89.21268

				203.26		89.18666

				203.28		89.17105

				203.3		89.11901

				203.32		89.1034

				203.34		89.1034

				203.36		89.09819

				203.38		89.08258

				203.4		89.06177

				203.43		89.05656

				203.45		89.04616

				203.47		89.04095

				203.49		89.02014

				203.51		89.00973

				203.53		88.99932

				203.55		88.98892

				203.57		88.9681

				203.59		88.97851

				203.61		88.9681

				203.63		88.95769

				203.66		88.94729

				203.68		88.94729

				203.7		88.91086

				203.72		88.90566

				203.74		88.89525

				203.76		88.88484

				203.78		88.88484

				203.8		88.89005

				203.82		88.85882

				203.84		88.83801

				203.86		88.83801

				203.88		88.81199

				203.91		88.76516

				203.93		88.77036

				203.95		88.76516

				203.97		88.73393

				203.99		88.71832

				204.01		88.73393

				204.03		88.72353

				204.05		88.70791

				204.07		88.6871

				204.09		88.69751

				204.11		88.67149

				204.14		88.65588

				204.16		88.64027

				204.18		88.65067

				204.2		88.60904

				204.22		88.60384

				204.24		88.61945

				204.26		88.60384

				204.28		88.58303

				204.3		88.58823

				204.32		88.58303

				204.34		88.53619

				204.37		88.5466

				204.39		88.53099

				204.41		88.51017

				204.43		88.48936

				204.45		88.50497

				204.47		88.47375

				204.49		88.45293

				204.51		88.45293

				204.53		88.44252

				204.55		88.41651

				204.57		88.4113

				204.59		88.4061

				204.62		88.38528

				204.64		88.37488

				204.66		88.35406

				204.68		88.33325

				204.7		88.31243

				204.72		88.29682

				204.74		88.29682

				204.76		88.28641

				204.78		88.27601

				204.8		88.2656

				204.82		88.23958

				204.85		88.21876

				204.87		88.22917

				204.89		88.22397

				204.91		88.20836

				204.93		88.21356

				204.95		88.19795

				204.97		88.17193

				204.99		88.16152

				205.01		88.15632

				205.03		88.14071

				205.05		88.1303

				205.07		88.11989

				205.1		88.10949

				205.12		88.08867

				205.14		88.07306

				205.16		88.06265

				205.18		88.05225

				205.2		88.02623

				205.22		88.02102

				205.24		88.01582

				205.26		87.9898

				205.28		88.00021

				205.3		87.995

				205.33		87.97419

				205.35		87.96899

				205.37		87.96378

				205.39		87.92736

				205.41		87.91174

				205.43		87.90134

				205.45		87.89613

				205.47		87.88573

				205.49		87.87012

				205.51		87.86491

				205.53		87.8441

				205.56		87.81808

				205.58		87.82328

				205.6		87.83369

				205.62		87.80767

				205.64		87.80767

				205.66		87.80247

				205.68		87.76604

				205.7		87.73482

				205.72		87.73482

				205.74		87.7036

				205.76		87.68798

				205.78		87.67237

				205.81		87.66717

				205.83		87.65156

				205.85		87.64115

				205.87		87.66717

				205.89		87.66717

				205.91		87.53708

				205.93		87.37576

				205.95		87.25608

				205.97		87.152

				205.99		87.11037

				206.01		87.23006

				206.04		87.34974

				206.06		87.433

				206.08		87.46943

				206.1		87.47463

				206.12		87.43821

				206.14		87.433

				206.16		87.43821

				206.18		87.42259

				206.2		87.41739

				206.22		87.41219

				206.24		87.40178

				206.26		87.36535

				206.29		87.37576

				206.31		87.36015

				206.33		87.36015

				206.35		87.31852

				206.37		87.34454

				206.39		87.30811

				206.41		87.29771

				206.43		87.27169

				206.45		87.30291

				206.47		87.27689

				206.49		87.27689

				206.51		87.28209

				206.54		87.30291

				206.56		87.30291

				206.58		87.32893

				206.6		87.37056

				206.62		87.39137

				206.64		87.39137

				206.66		87.35495

				206.68		87.30291

				206.7		87.23526

				206.72		87.16761

				206.74		87.11037

				206.76		87.07915

				206.79		87.05833

				206.81		87.03752

				206.83		87.0063

				206.85		86.99069

				206.87		86.97507

				206.89		86.94906

				206.91		86.93344

				206.93		86.93865

				206.95		86.93865

				206.97		86.92824

				206.99		86.92304

				207.02		86.91263

				207.04		86.89702

				207.06		86.8658

				207.08		86.8762

				207.1		86.84498

				207.12		86.83978

				207.14		86.82417

				207.16		86.82417

				207.18		86.77733

				207.2		86.76693

				207.22		86.75131

				207.25		86.74611

				207.27		86.7253

				207.29		86.71489

				207.31		86.70448

				207.33		86.68887

				207.35		86.66285

				207.37		86.66285

				207.39		86.65765

				207.41		86.63163

				207.43		86.61602

				207.45		86.61081

				207.48		86.57439

				207.5		86.55357

				207.52		86.56918

				207.54		86.55357

				207.56		86.52755

				207.58		86.52755

				207.6		86.51194

				207.62		86.48592

				207.64		86.47031

				207.66		86.4495

				207.68		86.42868

				207.71		86.41828

				207.73		86.40266

				207.75		86.41307

				207.77		86.40266

				207.79		86.39746

				207.81		86.39226

				207.83		86.37144

				207.85		86.32981

				207.87		86.33502

				207.89		86.309

				207.91		86.30379

				207.94		86.28298

				207.96		86.27777

				207.98		86.25176

				208		86.25696

				208.02		86.23615

				208.04		86.23094

				208.06		86.21013

				208.08		86.18931

				208.1		86.18931

				208.12		86.1685

				208.14		86.15289

				208.17		86.13207

				208.19		86.13727

				208.21		86.07483

				208.23		86.08003

				208.25		86.0384

				208.27		86.0384

				208.29		86.00198

				208.31		86.01759

				208.33		85.99157

				208.35		85.98637

				208.37		85.96035

				208.39		85.96035

				208.42		85.92392

				208.44		85.91351

				208.46		85.91872

				208.48		85.90311

				208.5		85.8875

				208.52		85.8875

				208.54		85.87709

				208.56		85.84066

				208.58		85.85627

				208.6		85.83025

				208.62		85.81464

				208.64		85.78862

				208.67		85.80424

				208.69		85.74179

				208.71		85.74179

				208.73		85.72618

				208.75		85.73659

				208.77		85.67414

				208.79		85.68975

				208.81		85.67935

				208.83		85.65333

				208.85		85.62211

				208.87		85.63772

				208.9		85.6169

				208.92		85.56486

				208.94		85.57527

				208.96		85.55446

				208.98		85.52844

				209		85.49201

				209.02		85.52323

				209.04		85.49722

				209.06		85.48681

				209.08		85.4712

				209.1		85.49201

				209.12		85.43998

				209.15		85.41916

				209.17		85.42436

				209.19		85.40875

				209.21		85.37233

				209.23		85.37753

				209.25		85.38794

				209.27		85.3359

				209.29		85.32029

				209.31		85.31509

				209.33		85.30988

				209.35		85.23703

				209.38		85.26825

				209.4		85.25264

				209.42		85.24223

				209.44		85.21101

				209.46		85.24744

				209.48		85.20581

				209.5		85.18499

				209.52		85.17979

				209.54		85.1954

				209.56		85.15897

				209.58		85.15377

				209.61		85.15377

				209.63		85.12775

				209.65		85.07571

				209.67		85.08612

				209.69		85.08092

				209.71		85.03929

				209.73		85.02888

				209.75		85.01847

				209.77		84.98205

				209.79		84.93001

				209.81		84.94042

				209.84		84.90399

				209.86		84.87797

				209.88		84.87797

				209.9		84.88318

				209.92		84.85195

				209.94		84.85716

				209.96		84.85195

				209.98		84.82073

				210		84.82594

				210.02		84.80512

				210.04		84.79471

				210.07		84.76349

				210.09		84.78431

				210.11		84.74268

				210.13		84.72186

				210.15		84.69584

				210.17		84.70625

				210.19		84.65421

				210.21		84.6438

				210.23		84.6438

				210.25		84.62819

				210.27		84.58656

				210.3		84.57616

				210.32		84.56575

				210.34		84.52932

				210.36		84.51371

				210.38		84.51371

				210.4		84.4981

				210.42		84.45647

				210.44		84.46688

				210.46		84.46167

				210.48		84.43566

				210.5		84.41484

				210.52		84.44086

				210.55		84.39403

				210.57		84.36801

				210.59		84.36801

				210.61		84.37841

				210.63		84.32117

				210.65		84.32638

				210.67		84.33679

				210.69		84.30036

				210.71		84.23791

				210.73		84.25873

				210.75		84.23271

				210.77		84.18588

				210.8		84.18067

				210.82		84.18588

				210.84		84.15465

				210.86		84.14425

				210.88		84.14945

				210.9		84.12864

				210.92		84.10782

				210.94		84.09221

				210.96		84.10262

				210.98		84.06619

				211		84.04017

				211.03		84.04017

				211.05		84.01415

				211.07		83.97773

				211.09		83.98293

				211.11		83.98293

				211.13		83.93089

				211.15		83.9361

				211.17		83.92049

				211.19		83.88926

				211.21		83.86325

				211.23		83.86845

				211.25		83.83202

				211.28		83.80601

				211.3		83.7956

				211.32		83.79039

				211.34		83.74876

				211.36		83.74876

				211.38		83.74356

				211.4		83.72795

				211.42		83.68632

				211.44		83.70193

				211.46		83.68632

				211.48		83.6603

				211.51		83.6655

				211.53		83.6551

				211.55		83.62387

				211.57		83.58745

				211.59		83.58745

				211.61		83.56143

				211.63		83.54062

				211.65		83.53021

				211.67		83.54582

				211.69		83.49899

				211.71		83.46256

				211.74		83.46256

				211.76		83.44695

				211.78		83.39491

				211.8		83.40011

				211.82		83.3845

				211.84		83.33767

				211.86		83.33767

				211.88		83.34287

				211.9		83.32206

				211.92		83.31165

				211.94		83.31685

				211.97		83.28563

				211.99		83.25961

				212.01		83.244

				212.03		83.2388

				212.05		83.22319

				212.07		83.19197

				212.09		83.17115

				212.11		83.15554

				212.13		83.11391

				212.15		83.1035

				212.17		83.08269

				212.19		83.06708

				212.22		83.04626

				212.24		83.05146

				212.26		83.01504

				212.28		83.00463

				212.3		82.98902

				212.32		82.97861

				212.34		82.963

				212.36		82.95259

				212.38		82.94219

				212.4		82.92137

				212.42		82.90576

				212.45		82.87974

				212.47		82.87974

				212.49		82.84852

				212.51		82.83811

				212.53		82.8277

				212.55		82.80169

				212.57		82.76526

				212.59		82.76526

				212.61		82.75485

				212.63		82.71322

				212.65		82.71843

				212.67		82.71322

				212.7		82.69241

				212.72		82.65078

				212.74		82.65598

				212.76		82.61956

				212.78		82.58313

				212.8		82.57793

				212.82		82.57793

				212.84		82.53109

				212.86		82.5363

				212.88		82.5467

				212.9		82.51028

				212.93		82.47385

				212.95		82.49467

				212.97		82.47906

				212.99		82.43743

				213.01		82.42702

				213.03		82.43743

				213.05		82.401

				213.07		82.36457

				213.09		82.36457

				213.11		82.34896

				213.13		82.31254

				213.15		82.30213

				213.18		82.30733

				213.2		82.27611

				213.22		82.23968

				213.24		82.23968

				213.26		82.21366

				213.28		82.18244

				213.3		82.15122

				213.32		82.15122

				213.34		82.10439

				213.36		82.09918

				213.38		82.08878

				213.41		82.08357

				213.43		82.05235

				213.45		82.07316

				213.47		82.04715

				213.49		82.01592

				213.51		82.01592

				213.53		82.01072

				213.55		81.97429

				213.57		81.95348

				213.59		81.94827

				213.61		81.90144

				213.64		81.89624

				213.66		81.88063

				213.68		81.86502

				213.7		81.81818

				213.72		81.839

				213.74		81.80777

				213.76		81.76094

				213.78		81.75053

				213.8		81.75574

				213.82		81.71411

				213.84		81.67768

				213.87		81.7089

				213.89		81.67768

				213.91		81.64646

				213.93		81.61003

				213.95		81.63085

				213.97		81.558

				213.99		81.53718

				214.01		81.53198

				214.03		81.54238

				214.05		81.49035

				214.07		81.50075

				214.1		81.48514

				214.12		81.45392

				214.14		81.40709

				214.16		81.39668

				214.18		81.37066

				214.2		81.33944

				214.22		81.31862

				214.24		81.31862

				214.26		81.2874

				214.28		81.26659

				214.3		81.27179

				214.32		81.25098

				214.35		81.21975

				214.37		81.20935

				214.39		81.22496

				214.41		81.18333

				214.43		81.17812

				214.45		81.17292

				214.47		81.16251

				214.49		81.11568

				214.51		81.11048

				214.53		81.07405

				214.55		81.05844

				214.58		81.02722

				214.6		81.01681

				214.62		80.99079

				214.64		80.96477

				214.66		80.94916

				214.68		80.92834

				214.7		80.90233

				214.72		80.8711

				214.74		80.8659

				214.76		80.81907

				214.78		80.81386

				214.8		80.78264

				214.83		80.77744

				214.85		80.75662

				214.87		80.77223

				214.89		80.74621

				214.91		80.73581

				214.93		80.70979

				214.95		80.69418

				214.97		80.66295

				214.99		80.63694

				215.01		80.63173

				215.03		80.62132

				215.06		80.5849

				215.08		80.55888

				215.1		80.56408

				215.12		80.50164

				215.14		80.50164

				215.16		80.50164

				215.18		80.47042

				215.2		80.43399

				215.22		80.45481

				215.24		80.41838

				215.26		80.37675

				215.28		80.35073

				215.31		80.36634

				215.33		80.32992

				215.35		80.29869

				215.37		80.31951

				215.39		80.31951

				215.41		80.26747

				215.43		80.25706

				215.45		80.25706

				215.47		80.20503

				215.49		80.1686

				215.51		80.1634

				215.54		80.13738

				215.56		80.09054

				215.58		80.09575

				215.6		80.06973

				215.62		80.03851

				215.64		80.01249

				215.66		80.00729

				215.68		79.99167

				215.7		79.97086

				215.72		79.95525

				215.74		79.94484

				215.76		79.92923

				215.79		79.8876

				215.81		79.90321

				215.83		79.87719

				215.85		79.84597

				215.87		79.81995

				215.89		79.81995

				215.91		79.76791

				215.93		79.7471

				215.95		79.73149

				215.97		79.72108

				215.99		79.68986

				216.02		79.66384

				216.04		79.65864

				216.06		79.63782

				216.08		79.6118

				216.1		79.59099

				216.12		79.58578

				216.14		79.54936

				216.16		79.54415

				216.18		79.50773

				216.2		79.49212

				216.22		79.4661

				216.25		79.45569

				216.27		79.42447

				216.29		79.42447

				216.31		79.41406

				216.33		79.38804

				216.35		79.36723

				216.37		79.36723

				216.39		79.336

				216.41		79.31519

				216.43		79.30999

				216.45		79.27356

				216.47		79.25274

				216.5		79.23193

				216.52		79.20591

				216.54		79.16949

				216.56		79.16428

				216.58		79.13306

				216.6		79.11745

				216.62		79.07582

				216.64		79.07582

				216.66		79.0498

				216.68		79.01337

				216.7		78.99256

				216.73		79.00297

				216.75		78.96134

				216.77		78.94573

				216.79		78.94052

				216.81		78.93011

				216.83		78.89889

				216.85		78.87287

				216.87		78.85206

				216.89		78.83124

				216.91		78.79482

				216.93		78.78961

				216.95		78.76359

				216.98		78.74278

				217		78.72196

				217.02		78.71156

				217.04		78.66993

				217.06		78.65432

				217.08		78.64391

				217.1		78.60748

				217.12		78.58667

				217.14		78.56585

				217.16		78.54504

				217.18		78.52422

				217.21		78.51382

				217.23		78.493

				217.25		78.47739

				217.27		78.45657

				217.29		78.42535

				217.31		78.41495

				217.33		78.37332

				217.35		78.3577

				217.37		78.33689

				217.39		78.31087

				217.41		78.29006

				217.43		78.27444

				217.46		78.23281

				217.48		78.23281

				217.5		78.212

				217.52		78.18598

				217.54		78.16517

				217.56		78.15996

				217.58		78.11833

				217.6		78.10272

				217.62		78.08191

				217.64		78.0767

				217.66		78.05589

				217.69		78.03507

				217.71		78.01426

				217.73		77.99344

				217.75		77.95702

				217.77		77.9362

				217.79		77.92059

				217.81		77.87376

				217.83		77.85294

				217.85		77.82172

				217.87		77.80091

				217.89		77.76448

				217.91		77.77489

				217.94		77.74366

				217.96		77.72805

				217.98		77.69683

				218		77.68122

				218.02		77.6552

				218.04		77.62918

				218.06		77.61357

				218.08		77.59276

				218.1		77.57194

				218.12		77.55113

				218.14		77.54592

				218.16		77.5147

				218.19		77.49909

				218.21		77.47307

				218.23		77.44185

				218.25		77.41583

				218.27		77.41063

				218.29		77.38461

				218.31		77.36379

				218.33		77.33257

				218.35		77.31696

				218.37		77.29094

				218.39		77.27013

				218.42		77.25972

				218.44		77.22329

				218.46		77.19207

				218.48		77.16605

				218.5		77.14003

				218.52		77.088

				218.54		77.10361

				218.56		77.08279

				218.58		77.05677

				218.6		77.03075

				218.62		77.04116

				218.64		76.99953

				218.67		76.98392

				218.69		76.9527

				218.71		76.93709

				218.73		76.90066

				218.75		76.86944

				218.77		76.85383

				218.79		76.82781

				218.81		76.79659

				218.83		76.79138

				218.85		76.75496

				218.87		76.70292

				218.89		76.70292

				218.92		76.6821

				218.94		76.65088

				218.96		76.62486

				218.98		76.64568

				219		76.59884

				219.02		76.58844

				219.04		76.54681

				219.06		76.55201

				219.08		76.50518

				219.1		76.49477

				219.12		76.46875

				219.15		76.45834

				219.17		76.41671

				219.19		76.40631

				219.21		76.38549

				219.23		76.34907

				219.25		76.32305

				219.27		76.30744

				219.29		76.2606

				219.31		76.22938

				219.33		76.21897

				219.35		76.18775

				219.37		76.16694

				219.4		76.16173

				219.42		76.14092

				219.44		76.08888

				219.46		76.08368

				219.48		76.06286

				219.5		76.02643

				219.52		75.99001

				219.54		76.02123

				219.56		75.9744

				219.58		75.94318

				219.6		75.93797

				219.63		75.93277

				219.65		75.87553

				219.67		75.86512

				219.69		75.85471

				219.71		75.79747

				219.73		75.77666

				219.75		75.75584

				219.77		75.74543

				219.79		75.68819

				219.81		75.68819

				219.83		75.66217

				219.86		75.62575

				219.88		75.58932

				219.9		75.59453

				219.92		75.5633

				219.94		75.54249

				219.96		75.53728

				219.98		75.52167

				220		75.48525

				220.02		75.46443

				220.04		75.46964

				220.06		75.4176

				220.09		75.38638

				220.11		75.37077

				220.13		75.35515

				220.15		75.2823

				220.17		75.28751

				220.19		75.24588

				220.21		75.22506

				220.23		75.16262

				220.25		75.16262

				220.27		75.13139

				220.29		75.12619

				220.31		75.08456

				220.34		75.09497

				220.36		75.04813

				220.38		75.02732

				220.4		75.01171

				220.42		74.99089

				220.44		74.98049

				220.46		74.95967

				220.48		74.95447

				220.5		74.90243

				220.52		74.90243

				220.54		74.866

				220.57		74.85039

				220.59		74.80356

				220.61		74.79315

				220.63		74.74632

				220.65		74.7203

				220.67		74.69948

				220.69		74.70469

				220.71		74.66306

				220.73		74.65265

				220.75		74.63184

				220.77		74.585

				220.8		74.53297

				220.82		74.51735

				220.84		74.49654

				220.86		74.4393

				220.88		74.44971

				220.9		74.42369

				220.92		74.39767

				220.94		74.37165

				220.96		74.38206

				220.98		74.33522

				221		74.30921

				221.03		74.28839

				221.05		74.28319

				221.07		74.22595

				221.09		74.20513

				221.11		74.18952

				221.13		74.1635

				221.15		74.11146

				221.17		74.11146

				221.19		74.09585

				221.21		74.06463

				221.23		74.04902

				221.25		74.023

				221.28		73.98657

				221.3		73.95015

				221.32		73.93974

				221.34		73.90852

				221.36		73.89291

				221.38		73.86168

				221.4		73.86689

				221.42		73.82006

				221.44		73.79404

				221.46		73.78363

				221.48		73.76281

				221.51		73.71598

				221.53		73.70557

				221.55		73.68996

				221.57		73.62752

				221.59		73.6067

				221.61		73.57548

				221.63		73.54426

				221.65		73.49222

				221.67		73.49742

				221.69		73.45059

				221.71		73.43498

				221.74		73.40376

				221.76		73.40376

				221.78		73.36213

				221.8		73.36213

				221.82		73.34131

				221.84		73.3205

				221.86		73.28407

				221.88		73.25805

				221.9		73.24244

				221.92		73.20602

				221.94		73.17479

				221.96		73.15918

				221.99		73.14357

				222.01		73.10714

				222.03		73.09674

				222.05		73.07072

				222.07		73.03429

				222.09		72.99787

				222.11		72.98226

				222.13		72.93022

				222.15		72.9094

				222.17		72.88859

				222.19		72.84696

				222.22		72.80533

				222.24		72.78451

				222.26		72.7585

				222.28		72.71166

				222.3		72.70646

				222.32		72.68044

				222.34		72.66483

				222.36		72.60759

				222.38		72.6232

				222.4		72.59198

				222.42		72.56596

				222.45		72.51392

				222.47		72.51912

				222.49		72.46188

				222.51		72.43066

				222.53		72.41505

				222.55		72.40464

				222.57		72.38903

				222.59		72.36301

				222.61		72.3526

				222.63		72.31097

				222.65		72.27455

				222.68		72.23812

				222.7		72.22251

				222.72		72.15486

				222.74		72.14446

				222.76		72.12364

				222.78		72.10283

				222.8		72.05599

				222.82		72.0716

				222.84		72.03518

				222.86		72.00395

				222.88		71.97794

				222.91		71.97273

				222.93		71.9311

				222.95		71.89988

				222.97		71.88947

				222.99		71.84264

				223.01		71.80101

				223.03		71.77499

				223.05		71.77499

				223.07		71.72295

				223.09		71.71775

				223.11		71.70214

				223.14		71.67092

				223.16		71.61888

				223.18		71.60327

				223.2		71.55643

				223.22		71.5148

				223.24		71.48358

				223.26		71.46277

				223.28		71.44195

				223.3		71.40553

				223.32		71.40032

				223.34		71.37951

				223.37		71.33788

				223.39		71.31186

				223.41		71.30666

				223.43		71.24941

				223.45		71.2234

				223.47		71.2234

				223.49		71.19738

				223.51		71.16095

				223.53		71.14014

				223.55		71.11932

				223.57		71.07769

				223.6		71.03606

				223.62		71.02045

				223.64		70.98923

				223.66		70.93199

				223.68		70.91117

				223.7		70.88515

				223.72		70.84873

				223.74		70.80189

				223.76		70.80189

				223.78		70.77588

				223.81		70.73425

				223.83		70.71343

				223.85		70.71343

				223.87		70.6666

				223.89		70.63017

				223.91		70.61456

				223.93		70.58854

				223.95		70.54171

				223.97		70.5365

				223.99		70.5365

				224.01		70.50528

				224.04		70.46886

				224.06		70.46365

				224.08		70.42723

				224.1		70.38039

				224.12		70.36478

				224.14		70.33876

				224.16		70.30754

				224.18		70.27111

				224.2		70.2451

				224.22		70.20347

				224.24		70.17224

				224.27		70.13582

				224.29		70.09939

				224.31		70.06817

				224.33		70.04735

				224.35		70.03695

				224.37		69.98491

				224.39		69.9693

				224.41		69.94848

				224.43		69.91726

				224.45		69.88604

				224.48		69.89124

				224.5		69.85482

				224.52		69.81839

				224.54		69.79758

				224.56		69.78196

				224.58		69.75074

				224.6		69.70391

				224.62		69.70911

				224.64		69.65707

				224.66		69.60504

				224.68		69.57902

				224.71		69.56861

				224.73		69.50617

				224.75		69.48535

				224.77		69.46974

				224.79		69.42811

				224.81		69.37087

				224.83		69.37087

				224.85		69.35005

				224.87		69.30842

				224.89		69.28761

				224.92		69.31363

				224.94		69.25639

				224.96		69.21996

				224.98		69.19915

				225		69.17833

				225.02		69.10548

				225.04		69.09507

				225.06		69.07946

				225.08		69.03783

				225.1		68.9962

				225.13		68.98059

				225.15		68.95978

				225.17		68.90774

				225.19		68.89733

				225.21		68.87131

				225.23		68.83489

				225.25		68.78805

				225.27		68.77764

				225.29		68.73081

				225.31		68.68398

				225.33		68.66837

				225.36		68.64755

				225.38		68.61633

				225.4		68.5799

				225.42		68.58511

				225.44		68.53827

				225.46		68.50705

				225.48		68.48103

				225.5		68.46022

				225.52		68.41338

				225.54		68.40298

				225.56		68.38216

				225.59		68.34574

				225.61		68.30931

				225.63		68.28849

				225.65		68.23646

				225.67		68.20003

				225.69		68.17401

				225.71		68.14279

				225.73		68.09596

				225.75		68.09075

				225.77		68.06473

				225.8		68.0179

				225.82		67.98147

				225.84		67.97627

				225.86		67.93464

				225.88		67.8826

				225.9		67.8722

				225.92		67.84618

				225.94		67.79934

				225.96		67.77333

				225.98		67.76292

				226		67.71088

				226.03		67.67966

				226.05		67.64844

				226.07		67.61721

				226.09		67.57038

				226.11		67.54436

				226.13		67.53916

				226.15		67.51314

				226.17		67.46631

				226.19		67.4559

				226.21		67.42468

				226.24		67.36744

				226.26		67.34142

				226.28		67.3206

				226.3		67.26336

				226.32		67.22173

				226.34		67.22173

				226.36		67.1853

				226.38		67.13327

				226.4		67.12806

				226.42		67.11766

				226.44		67.06562

				226.47		67.02399

				226.49		67.00838

				226.51		66.98236

				226.53		66.92512

				226.55		66.8939

				226.57		66.87308

				226.59		66.84706

				226.61		66.80543

				226.63		66.77941

				226.65		66.74819

				226.68		66.69615

				226.7		66.66493

				226.72		66.61289

				226.74		66.59208

				226.76		66.54525

				226.78		66.54004

				226.8		66.49841

				226.82		66.47239

				226.84		66.44117

				226.86		66.41515

				226.88		66.37352

				226.91		66.33189

				226.93		66.32149

				226.95		66.28506

				226.97		66.24863

				226.99		66.23823

				227.01		66.22262

				227.03		66.18619

				227.05		66.16017

				227.07		66.13936

				227.09		66.08211

				227.11		66.03528

				227.14		66.01447

				227.16		65.98324

				227.18		65.94682

				227.2		65.93641

				227.22		65.90519

				227.24		65.86876

				227.26		65.84274

				227.28		65.81672

				227.3		65.77509

				227.32		65.73867

				227.35		65.71785

				227.37		65.67102

				227.39		65.65021

				227.41		65.60337

				227.43		65.59296

				227.45		65.55133

				227.47		65.51491

				227.49		65.47848

				227.51		65.45767

				227.53		65.41604

				227.55		65.38482

				227.58		65.3692

				227.6		65.30156

				227.62		65.25993

				227.64		65.24952

				227.66		65.19748

				227.68		65.16626

				227.7		65.16626

				227.72		65.13504

				227.74		65.06218

				227.76		65.06218

				227.78		65.01535

				227.81		64.97892

				227.83		64.9477

				227.85		64.9373

				227.87		64.88526

				227.89		64.84883

				227.91		64.8072

				227.93		64.79159

				227.95		64.74476

				227.97		64.69792

				227.99		64.68231

				228.01		64.6667

				228.04		64.60946

				228.06		64.59905

				228.08		64.57303

				228.1		64.5314

				228.12		64.49498

				228.14		64.46376

				228.16		64.41692

				228.18		64.37529

				228.2		64.34927

				228.22		64.31805

				228.24		64.28683

				228.27		64.2452

				228.29		64.23479

				228.31		64.17755

				228.33		64.15153

				228.35		64.12551

				228.37		64.1099

				228.39		64.05266

				228.41		64.04746

				228.43		64.00062

				228.45		63.95899

				228.47		63.92777

				228.5		63.90696

				228.52		63.86533

				228.54		63.83931

				228.56		63.8237

				228.58		63.77166

				228.6		63.76125

				228.62		63.71442

				228.64		63.6884

				228.66		63.63116

				228.68		63.61035

				228.7		63.55831

				228.73		63.52709

				228.75		63.46984

				228.77		63.47505

				228.79		63.43342

				228.81		63.36577

				228.83		63.34495

				228.85		63.32934

				228.87		63.2669

				228.89		63.23568

				228.91		63.24608

				228.93		63.20445

				228.96		63.15762

				228.98		63.14201

				229		63.11599

				229.02		63.06916

				229.04		63.02232

				229.06		63.02232

				229.08		62.97549

				229.1		62.91305

				229.12		62.88703

				229.14		62.86101

				229.17		62.79336

				229.19		62.75173

				229.21		62.73612

				229.23		62.69969

				229.25		62.64766

				229.27		62.63725

				229.29		62.60082

				229.31		62.54878

				229.33		62.51756

				229.35		62.50716

				229.37		62.46553

				229.4		62.44471

				229.42		62.4239

				229.44		62.40308

				229.46		62.35104

				229.48		62.31982

				229.5		62.28339

				229.52		62.25217

				229.54		62.20534

				229.56		62.15851

				229.58		62.12208

				229.6		62.06484

				229.63		62.03362

				229.65		61.99199

				229.67		61.96076

				229.69		61.92954

				229.71		61.91393

				229.73		61.85669

				229.75		61.82026

				229.77		61.77863

				229.79		61.737

				229.81		61.70058

				229.83		61.67976

				229.86		61.65374

				229.88		61.62252

				229.9		61.5913

				229.92		61.56008

				229.94		61.50284

				229.96		61.46641

				229.98		61.4456

				230		61.40397

				230.02		61.36754

				230.04		61.34152

				230.06		61.30509

				230.09		61.26346

				230.11		61.22183

				230.13		61.18541

				230.15		61.15419

				230.17		61.10215

				230.19		61.07613

				230.21		61.05532

				230.23		61.00848

				230.25		60.95644

				230.27		60.95644

				230.29		60.90441

				230.32		60.85237

				230.34		60.83156

				230.36		60.81074

				230.38		60.7535

				230.4		60.70667

				230.42		60.69626

				230.44		60.63902

				230.46		60.60259

				230.48		60.57137

				230.5		60.56096

				230.52		60.49852

				230.55		60.48291

				230.57		60.44128

				230.59		60.41005

				230.61		60.3372

				230.63		60.32679

				230.65		60.28516

				230.67		60.24874

				230.69		60.21231

				230.71		60.2019

				230.73		60.16548

				230.75		60.12905

				230.78		60.09263

				230.8		60.0562

				230.82		60.01457

				230.84		59.97294

				230.86		59.95213

				230.88		59.9157

				230.9		59.86887

				230.92		59.83244

				230.94		59.79601

				230.96		59.72837

				230.98		59.70755

				231.01		59.67112

				231.03		59.64511

				231.05		59.60868

				231.07		59.58266

				231.09		59.51501

				231.11		59.50461

				231.13		59.45777

				231.15		59.42135

				231.17		59.38492

				231.19		59.3641

				231.22		59.32247

				231.24		59.26003

				231.26		59.23401

				231.28		59.19759

				231.3		59.16116

				231.32		59.11433

				231.34		59.11433

				231.36		59.06229

				231.38		59.02586

				231.4		58.98944

				231.42		58.95821

				231.45		58.89057

				231.47		58.85414

				231.49		58.82292

				231.51		58.7969

				231.53		58.74486

				231.55		58.72405

				231.57		58.68242

				231.59		58.64079

				231.61		58.59916

				231.63		58.56273

				231.65		58.5263

				231.68		58.49508

				231.7		58.44825

				231.72		58.41703

				231.74		58.37019

				231.76		58.32336

				231.78		58.30775

				231.8		58.26091

				231.82		58.22449

				231.84		58.19327

				231.86		58.16204

				231.89		58.11001

				231.91		58.07878

				231.93		58.04236

				231.95		58.00073

				231.97		57.9643

				231.99		57.91747

				232.01		57.89665

				232.03		57.82901

				232.05		57.79778

				232.07		57.75615

				232.09		57.72493

				232.12		57.66769

				232.14		57.65728

				232.16		57.61045

				232.18		57.58443

				232.2		57.55321

				232.22		57.52719

				232.24		57.48036

				232.26		57.43873

				232.28		57.39189

				232.3		57.35547

				232.32		57.30863

				232.35		57.267

				232.37		57.24098

				232.39		57.19935

				232.41		57.14211

				232.43		57.11089

				232.45		57.07447

				232.47		57.02243

				232.49		56.986

				232.51		56.95478

				232.53		56.91315

				232.56		56.88193

				232.58		56.81948

				232.6		56.78306

				232.62		56.76224

				232.64		56.71541

				232.66		56.67898

				232.68		56.66337

				232.7		56.62694

				232.72		56.59052

				232.74		56.55409

				232.76		56.51246

				232.79		56.47083

				232.81		56.424

				232.83		56.37717

				232.85		56.34594

				232.87		56.29911

				232.89		56.25228

				232.91		56.21585

				232.93		56.19504

				232.95		56.13259

				232.97		56.11698

				233		56.04933

				233.02		56.02852

				233.04		55.97128

				233.06		55.94005

				233.08		55.8724

				233.1		55.8724

				233.12		55.81516

				233.14		55.78394

				233.16		55.73711

				233.18		55.71109

				233.2		55.66946

				233.23		55.62783

				233.25		55.5914

				233.27		55.56538

				233.29		55.52896

				233.31		55.47692

				233.33		55.4457

				233.35		55.38846

				233.37		55.35203

				233.39		55.3052

				233.41		55.27398

				233.43		55.21153

				233.46		55.18031

				233.48		55.12827

				233.5		55.08664

				233.52		55.05022

				233.54		55.00338

				233.56		54.97216

				233.58		54.93053

				233.6		54.90451

				233.62		54.86288

				233.64		54.84207

				233.67		54.79523

				233.69		54.77442

				233.71		54.72758

				233.73		54.68596

				233.75		54.64433

				233.77		54.62871

				233.79		54.56627

				233.81		54.52984

				233.83		54.48301

				233.85		54.44138

				233.87		54.38934

				233.9		54.35812

				233.92		54.29047

				233.94		54.25405

				233.96		54.22282

				233.98		54.17079

				234		54.11355

				234.02		54.09793

				234.04		54.06151

				234.06		54.02508

				234.08		53.97304

				234.1		53.94703

				234.13		53.89499

				234.15		53.83775

				234.17		53.80653

				234.19		53.78051

				234.21		53.73367

				234.23		53.69725

				234.25		53.67643

				234.27		53.61919

				234.29		53.57236

				234.31		53.53593

				234.34		53.49951

				234.36		53.43186

				234.38		53.39543

				234.4		53.3538

				234.42		53.31738

				234.44		53.26534

				234.46		53.23412

				234.48		53.19249

				234.5		53.14045

				234.52		53.08321

				234.55		53.05199

				234.57		53.01036

				234.59		52.96352

				234.61		52.9375

				234.63		52.90628

				234.65		52.84384

				234.67		52.7918

				234.69		52.76058

				234.71		52.71374

				234.73		52.6565

				234.75		52.63048

				234.78		52.59406

				234.8		52.52121

				234.82		52.48998

				234.84		52.46917

				234.86		52.39111

				234.88		52.35989

				234.9		52.34428

				234.92		52.28704

				234.94		52.22459

				234.96		52.21419

				234.99		52.16215

				235.01		52.11011

				235.03		52.07368

				235.05		52.02685

				235.07		51.98002

				235.09		51.94359

				235.11		51.91237

				235.13		51.88635

				235.15		51.83952

				235.17		51.78748

				235.19		51.75105

				235.22		51.69381

				235.24		51.63137

				235.26		51.60535

				235.28		51.56892

				235.3		51.51168

				235.32		51.48046

				235.34		51.44924

				235.36		51.37639

				235.38		51.35037

				235.4		51.30353

				235.42		51.2567

				235.45		51.18905

				235.47		51.17864

				235.49		51.13181

				235.51		51.06937

				235.53		51.04335

				235.55		51.02774

				235.57		50.96009

				235.59		50.91846

				235.61		50.87162

				235.63		50.82999

				235.66		50.77275

				235.68		50.77275

				235.7		50.71551

				235.72		50.68949

				235.74		50.62705

				235.76		50.58542

				235.78		50.52297

				235.8		50.48134

				235.82		50.43971

				235.84		50.39809

				235.86		50.35646

				235.89		50.30442

				235.91		50.2784

				235.93		50.21075

				235.95		50.17432

				235.97		50.12749

				235.99		50.08066

				236.01		50.02342

				236.03		50.00781

				236.05		49.95577

				236.07		49.90373

				236.09		49.87251

				236.12		49.83088

				236.14		49.78405

				236.16		49.73721

				236.18		49.70599

				236.2		49.66436

				236.22		49.60712

				236.24		49.56029

				236.26		49.51345

				236.28		49.46141

				236.3		49.40417

				236.33		49.38856

				236.35		49.32612

				236.37		49.2949

				236.39		49.24806

				236.41		49.21164

				236.43		49.14399

				236.45		49.09715

				236.47		49.08154

				236.49		49.03471

				236.51		48.98788

				236.53		48.95665

				236.56		48.92543

				236.58		48.85778

				236.6		48.81615

				236.62		48.77973

				236.64		48.73289

				236.66		48.68086

				236.68		48.66004

				236.7		48.62361

				236.72		48.56117

				236.74		48.51434

				236.76		48.48832

				236.79		48.41547

				236.81		48.35302

				236.83		48.33221

				236.85		48.25935

				236.87		48.21252

				236.89		48.17609

				236.91		48.13446

				236.93		48.06682

				236.95		48.02519

				236.97		47.99917

				237		47.94713

				237.02		47.88989

				237.04		47.86387

				237.06		47.84826

				237.08		47.765

				237.1		47.72337

				237.12		47.70256

				237.14		47.63491

				237.16		47.57767

				237.18		47.56205

				237.2		47.50481

				237.23		47.45798

				237.25		47.42155

				237.27		47.40074

				237.29		47.31748

				237.31		47.28105

				237.33		47.22902

				237.35		47.16657

				237.37		47.10933

				237.39		47.08331

				237.41		47.04689

				237.44		46.97403

				237.46		46.94801

				237.48		46.90638

				237.5		46.85435

				237.52		46.7815

				237.54		46.7919

				237.56		46.72946

				237.58		46.66701

				237.6		46.61498

				237.62		46.58375

				237.64		46.5057

				237.67		46.46407

				237.69		46.43285

				237.71		46.3756

				237.73		46.33918

				237.75		46.28714

				237.77		46.26112

				237.79		46.18827

				237.81		46.17266

				237.83		46.12583

				237.85		46.06338

				237.88		46.00614

				237.9		45.96451

				237.92		45.91247

				237.94		45.86564

				237.96		45.83442

				237.98		45.8084

				238		45.76157

				238.02		45.71994

				238.04		45.6679

				238.06		45.64188

				238.08		45.56903

				238.11		45.53781

				238.13		45.48056

				238.15		45.42332

				238.17		45.35567

				238.19		45.32445

				238.21		45.26721

				238.23		45.20997

				238.25		45.17875

				238.27		45.12151

				238.29		45.06427

				238.31		45.01743

				238.34		44.99141

				238.36		44.90295

				238.38		44.87693

				238.4		44.8301

				238.42		44.79367

				238.44		44.71562

				238.46		44.70001

				238.48		44.66358

				238.5		44.60634

				238.52		44.53869

				238.55		44.53349

				238.57		44.48145

				238.59		44.40339

				238.61		44.38778

				238.63		44.36176

				238.65		44.28891

				238.67		44.24208

				238.69		44.21085

				238.71		44.14321

				238.73		44.07035

				238.75		44.03393

				238.78		43.9975

				238.8		43.91945

				238.82		43.86741

				238.84		43.8518

				238.86		43.79976

				238.88		43.72691

				238.9		43.72691

				238.92		43.68528

				238.94		43.60202

				238.96		43.54998

				238.99		43.54478

				239.01		43.46152

				239.03		43.41989

				239.05		43.40948

				239.07		43.35224

				239.09		43.27939

				239.11		43.23255

				239.13		43.21694

				239.15		43.13368

				239.17		43.09205

				239.19		43.06083

				239.22		42.99318

				239.24		42.92033

				239.26		42.90992

				239.28		42.84228

				239.3		42.75902

				239.32		42.7434

				239.34		42.69657

				239.36		42.62372

				239.38		42.58729

				239.4		42.57168

				239.43		42.50403

				239.45		42.46761

				239.47		42.43118

				239.49		42.39475

				239.51		42.3219

				239.53		42.29588

				239.55		42.22824

				239.57		42.16579

				239.59		42.10335

				239.61		42.06692

				239.64		41.99407

				239.66		41.93683

				239.68		41.8952

				239.7		41.84836

				239.72		41.78592

				239.74		41.74949

				239.76		41.72347

				239.78		41.63501

				239.8		41.58818

				239.82		41.56216

				239.84		41.51012

				239.87		41.41645

				239.89		41.40084

				239.91		41.35921

				239.93		41.29156

				239.95		41.24473

				239.97		41.24473

				239.99		41.18229

				240.01		41.11984

				240.03		41.09382

				240.05		41.04699

				240.08		40.97414

				240.1		40.9221

				240.12		40.88567

				240.14		40.81282

				240.16		40.74517

				240.18		40.71915

				240.2		40.67232

				240.22		40.60467

				240.24		40.56825

				240.26		40.52141

				240.29		40.45376

				240.31		40.38091

				240.33		40.3601

				240.35		40.31326

				240.37		40.25082

				240.39		40.20399

				240.41		40.18837

				240.43		40.11032

				240.45		40.05828

				240.47		40.02706

				240.49		39.98023

				240.52		39.91258

				240.54		39.87615

				240.56		39.83452

				240.58		39.76167

				240.6		39.71484

				240.62		39.668

				240.64		39.61597

				240.66		39.54832

				240.68		39.5223

				240.7		39.46506

				240.72		39.40782

				240.75		39.36098

				240.77		39.32456

				240.79		39.25691

				240.81		39.19446

				240.83		39.16324

				240.85		39.1008

				240.87		39.04356

				240.89		38.99152

				240.91		38.98111

				240.93		38.90305

				240.95		38.87704

				240.98		38.81979

				241		38.79378

				241.02		38.70531

				241.04		38.67409

				241.06		38.59083

				241.08		38.52318

				241.1		38.45553

				241.12		38.42431

				241.14		38.33585

				241.16		38.29422

				241.19		38.2734

				241.21		38.22137

				241.23		38.14331

				241.25		38.1225

				241.27		38.07566

				241.29		37.99761

				241.31		37.96118

				241.33		37.91955

				241.35		37.86231

				241.37		37.78946

				241.39		37.77905

				241.42		37.7114

				241.44		37.65936

				241.46		37.60733

				241.48		37.5761

				241.5		37.49805

				241.52		37.44081

				241.54		37.40959

				241.56		37.35755

				241.58		37.2951

				241.6		37.24827

				241.62		37.21184

				241.65		37.12338

				241.67		37.07655

				241.69		37.02451

				241.71		36.98288

				241.73		36.89962

				241.75		36.87881

				241.77		36.82677

				241.79		36.76432

				241.81		36.70188

				241.83		36.69147

				241.86		36.61862

				241.88		36.55617

				241.9		36.51975

				241.92		36.47812

				241.94		36.40527

				241.96		36.35323

				241.98		36.32201

				242		36.26997

				242.02		36.20752

				242.04		36.15028

				242.06		36.10865

				242.09		36.0358

				242.11		35.98897

				242.13		35.92132

				242.15		35.87969

				242.17		35.81725

				242.19		35.78082

				242.21		35.71317

				242.23		35.66634

				242.25		35.6195

				242.27		35.56747

				242.3		35.50502

				242.32		35.43737

				242.34		35.41656

				242.36		35.34891

				242.38		35.31248

				242.4		35.25524

				242.42		35.21882

				242.44		35.14596

				242.46		35.10954

				242.48		35.03669

				242.5		34.98985

				242.53		34.9222

				242.55		34.88057

				242.57		34.80772

				242.59		34.75569

				242.61		34.70365

				242.63		34.66202

				242.65		34.58917

				242.67		34.54233

				242.69		34.4903

				242.71		34.42785

				242.73		34.37581

				242.76		34.33939

				242.78		34.28735

				242.8		34.2197

				242.82		34.17287

				242.84		34.12603

				242.86		34.06359

				242.88		33.99074

				242.9		33.95431

				242.92		33.90227

				242.94		33.82942

				242.97		33.77738

				242.99		33.74616

				243.01		33.6629

				243.03		33.60566

				243.05		33.56403

				243.07		33.49118

				243.09		33.43394

				243.11		33.38711

				243.13		33.33507

				243.15		33.25701

				243.17		33.21538

				243.2		33.16334

				243.22		33.12172

				243.24		33.05927

				243.26		33.02284

				243.28		32.97081

				243.3		32.91877

				243.32		32.83551

				243.34		32.78868

				243.36		32.73144

				243.38		32.69501

				243.41		32.61175

				243.43		32.60134

				243.45		32.53369

				243.47		32.47125

				243.49		32.3984

				243.51		32.36717

				243.53		32.28392

				243.55		32.23708

				243.57		32.19025

				243.59		32.13301

				243.61		32.07056

				243.64		32.02373

				243.66		31.96128

				243.68		31.91965

				243.7		31.87282

				243.72		31.80517

				243.74		31.76875

				243.76		31.7063

				243.78		31.64386

				243.8		31.57621

				243.82		31.55019

				243.85		31.46173

				243.87		31.4305

				243.89		31.35765

				243.91		31.32123

				243.93		31.24837

				243.95		31.20154

				243.97		31.1495

				243.99		31.12348

				244.01		31.05063

				244.03		30.98819

				244.06		30.95176

				244.08		30.8633

				244.1		30.80085

				244.12		30.74361

				244.14		30.70719

				244.16		30.61352

				244.18		30.5823

				244.2		30.51465

				244.22		30.45741

				244.24		30.38976

				244.26		30.35854

				244.29		30.3013

				244.31		30.23365

				244.33		30.18681

				244.35		30.12957

				244.37		30.06713

				244.39		29.98907

				244.41		29.97346

				244.43		29.90061

				244.45		29.84337

				244.47		29.77572

				244.5		29.72889

				244.52		29.66124

				244.54		29.6092

				244.56		29.54155

				244.58		29.51033

				244.6		29.43748

				244.62		29.36983

				244.64		29.323

				244.66		29.26575

				244.68		29.20331

				244.71		29.16168

				244.73		29.12005

				244.75		29.0524

				244.77		28.99516

				244.79		28.93792

				244.81		28.88068

				244.83		28.81303

				244.85		28.75059

				244.87		28.70896

				244.89		28.66212

				244.91		28.59447

				244.94		28.54764

				244.96		28.50081

				244.98		28.43836

				245		28.37592

				245.02		28.32388

				245.04		28.26144

				245.06		28.18338

				245.08		28.15216

				245.1		28.0741

				245.12		28.02206

				245.15		27.9388

				245.17		27.90238

				245.19		27.82432

				245.21		27.78269

				245.23		27.70464

				245.25		27.68903

				245.27		27.62138

				245.29		27.56934

				245.31		27.49649

				245.33		27.44965

				245.35		27.36639

				245.38		27.31436

				245.4		27.25191

				245.42		27.19988

				245.44		27.14263

				245.46		27.0906

				245.48		27.03336

				245.5		26.97611

				245.52		26.90326

				245.54		26.85123

				245.56		26.8148

				245.59		26.75235

				245.61		26.68991

				245.63		26.64308

				245.65		26.58584

				245.67		26.49737

				245.69		26.43493

				245.71		26.37769

				245.73		26.32045

				245.75		26.26841

				245.77		26.22678

				245.8		26.18515

				245.82		26.1227

				245.84		26.05506

				245.86		26.00822

				245.88		25.93537

				245.9		25.8417

				245.92		25.80007

				245.94		25.75324

				245.96		25.68559

				245.98		25.63355

				246		25.59713

				246.03		25.54509

				246.05		25.48265

				246.07		25.415

				246.09		25.37337

				246.11		25.31613

				246.13		25.24327

				246.15		25.18603

				246.17		25.1444

				246.19		25.05594

				246.21		24.9987

				246.24		24.94146

				246.26		24.88942

				246.28		24.82177

				246.3		24.76974

				246.32		24.70209

				246.34		24.65005

				246.36		24.5772

				246.38		24.52516

				246.4		24.46792

				246.42		24.42109

				246.45		24.34823

				246.47		24.3066

				246.49		24.21814

				246.51		24.18692

				246.53		24.11927

				246.55		24.04642

				246.57		23.98918

				246.59		23.94755

				246.61		23.87469

				246.63		23.81745

				246.66		23.7446

				246.68		23.67695

				246.7		23.62492

				246.72		23.54686

				246.74		23.48441

				246.76		23.4688

				246.78		23.40116

				246.8		23.34391

				246.82		23.29188

				246.84		23.24504

				246.86		23.16699

				246.89		23.12015

				246.91		23.05251

				246.93		22.99006

				246.95		22.91721

				246.97		22.86517

				246.99		22.79752

				247.01		22.75069

				247.03		22.68824

				247.05		22.6258

				247.07		22.55295

				247.1		22.49571

				247.12		22.42806

				247.14		22.35

				247.16		22.29797

				247.18		22.24072

				247.2		22.18348

				247.22		22.12104

				247.24		22.08461

				247.26		22.01176

				247.28		21.94932

				247.31		21.88167

				247.33		21.82443

				247.35		21.76719

				247.37		21.72035

				247.39		21.66311

				247.41		21.60587

				247.43		21.54343

				247.45		21.47578

				247.47		21.40292

				247.49		21.33528

				247.52		21.27804

				247.54		21.22079

				247.56		21.17396

				247.58		21.10111

				247.6		21.06989

				247.62		21.00744

				247.64		20.93459

				247.66		20.86174

				247.68		20.82011

				247.7		20.74205

				247.73		20.67961

				247.75		20.60155

				247.77		20.55992

				247.79		20.49748

				247.81		20.42983

				247.83		20.37779

				247.85		20.33616

				247.87		20.2529

				247.89		20.20086

				247.91		20.12801

				247.94		20.07077

				247.96		20.00312

				247.98		19.94068

				248		19.86783

				248.02		19.81579

				248.04		19.75334

				248.06		19.70131

				248.08		19.63886

				248.1		19.58682

				248.12		19.51918

				248.15		19.45673

				248.17		19.37868

				248.19		19.32143

				248.21		19.2746

				248.23		19.21216

				248.25		19.1341

				248.27		19.09247

				248.29		19.03003

				248.31		18.96238

				248.33		18.89473

				248.36		18.8531

				248.38		18.78545

				248.4		18.72301

				248.42		18.63975

				248.44		18.59291

				248.46		18.52006

				248.48		18.45762

				248.5		18.38997

				248.52		18.32752

				248.54		18.27549

				248.57		18.21304

				248.59		18.13498

				248.61		18.08295

				248.63		18.04132

				248.65		17.96326

				248.67		17.89041

				248.69		17.83837

				248.71		17.77072

				248.73		17.69787

				248.75		17.65104

				248.78		17.5938

				248.8		17.54176

				248.82		17.47411

				248.84		17.40646

				248.86		17.34402

				248.88		17.27637

				248.9		17.22433

				248.92		17.14628

				248.94		17.09424

				248.96		17.02139

				248.99		16.96415

				249.01		16.88089

				249.03		16.83405

				249.05		16.77161

				249.07		16.68835

				249.09		16.6155

				249.11		16.56866

				249.13		16.50101

				249.15		16.44377

				249.18		16.39174

				249.2		16.35531

				249.22		16.28246

				249.24		16.24083

				249.26		16.16277

				249.28		16.11594

				249.3		16.03788

				249.32		15.99105

				249.34		15.9182

				249.36		15.85575

				249.39		15.79851

				249.41		15.72046

				249.43		15.65281

				249.45		15.59557

				249.47		15.53833

				249.49		15.46547

				249.51		15.39782

				249.53		15.3562

				249.55		15.27814

				249.57		15.2209

				249.6		15.16886

				249.62		15.12723

				249.64		15.04397

				249.66		14.98153

				249.68		14.90867

				249.7		14.85143

				249.72		14.77858

				249.74		14.73175

				249.76		14.6693

				249.78		14.60165

				249.81		14.5236

				249.83		14.48717

				249.85		14.39871

				249.87		14.34667

				249.89		14.29984

				249.91		14.2478

				249.93		14.15413

				249.95		14.09689

				249.97		14.03445

				249.99		13.9616

				250.02		13.90436

				250.04		13.86273

				250.06		13.81069

				250.08		13.71182

				250.1		13.66498

				250.12		13.60774

				250.14		13.52448

				250.16		13.44643

				250.18		13.41521

				250.2		13.33715

				250.23		13.25909

				250.25		13.21746

				250.27		13.14982

				250.29		13.07696

				250.31		13.00931

				250.33		12.94687

				250.35		12.85841

				250.37		12.80637

				250.39		12.74392

				250.41		12.69709

				250.44		12.61904

				250.46		12.58261

				250.48		12.53057

				250.5		12.45772

				250.52		12.37966

				250.54		12.34844

				250.56		12.26518

				250.58		12.17672

				250.6		12.1455

				250.62		12.09866

				250.65		12.0102

				250.67		11.95816

				250.69		11.92694

				250.71		11.83327

				250.73		11.76562

				250.75		11.69798

				250.77		11.62512

				250.79		11.55227

				250.81		11.49503

				250.83		11.41697

				250.86		11.36494

				250.88		11.29729

				250.9		11.24525

				250.92		11.18281

				250.94		11.11516

				250.96		11.05792

				250.98		10.99547

				251		10.91742

				251.02		10.84456

				251.04		10.80293

				251.07		10.72488

				251.09		10.67805

				251.11		10.62601

				251.13		10.57917

				251.15		10.50112

				251.17		10.44388

				251.19		10.36582

				251.21		10.29297

				251.23		10.22012

				251.25		10.16808

				251.28		10.10043

				251.3		10.03799

				251.32		9.98595

				251.34		9.913098

				251.36		9.840246

				251.38		9.767393

				251.4		9.710152

				251.42		9.6373

				251.44		9.585263

				251.46		9.522818

				251.49		9.475985

				251.51		9.397929

				251.53		9.340688

				251.55		9.293854

				251.57		9.215799

				251.59		9.14815

				251.61		9.111724

				251.63		9.028464

				251.65		8.945205

				251.67		8.88276

				251.7		8.830723

				251.72		8.731852

				251.74		8.685018

				251.76		8.627777

				251.78		8.560129

				251.8		8.492481

				251.82		8.440443

				251.84		8.377999

				251.86		8.305146

				251.88		8.247906

				251.91		8.185461

				251.93		8.123016

				251.95		8.039756

				251.97		7.998127

				251.99		7.940886

				252.01		7.868034

				252.03		7.805589

				252.05		7.769163

				252.07		7.680699

				252.09		7.607847

				252.12		7.561014

				252.14		7.493365

				252.16		7.415309

				252.18		7.352865

				252.2		7.316439

				252.22		7.217568

				252.24		7.160327

				252.26		7.10829

				252.28		7.040641

				252.3		6.957381

				252.33		6.936567

				252.35		6.853307

				252.37		6.775251

				252.39		6.723214

				252.41		6.671177

				252.43		6.603528

				252.45		6.53588

				252.47		6.499454

				252.49		6.442213

				252.51		6.358953

				252.54		6.291305

				252.56		6.254878

				252.58		6.166415

				252.6		6.10397

				252.62		6.062341

				252.64		6.0051

				252.66		5.932247

				252.68		5.869803

				252.7		5.817766

				252.72		5.755321

				252.75		5.692876

				252.77		5.646043

				252.79		5.594005

				252.81		5.515949

				252.83		5.469116

				252.85		5.39106

				252.87		5.323412

				252.89		5.260967

				252.91		5.203726

				252.93		5.104855

				252.96		5.073633

				252.98		4.995577

				253		4.94354

				253.02		4.849873

				253.04		4.844669

				253.06		4.756205

				253.08		4.704168

				253.1		4.63652

				253.12		4.620909

				253.14		4.51163

				253.17		4.454389

				253.19		4.407556

				253.21		4.355519

				253.23		4.261851

				253.25		4.241037

				253.27		4.215018

				253.29		4.142166

				253.31		4.079721

				253.33		4.043295

				253.35		3.954832

				253.37		3.861165

				253.4		3.803924

				253.42		3.751886

				253.44		3.668627

				253.46		3.626997

				253.48		3.595775

				253.5		3.538534

				253.52		3.481293

				253.54		3.439663

				253.56		3.398033

				253.58		3.325181

				253.61		3.247125

				253.63		3.210699

				253.65		3.148254

				253.67		3.085809

				253.69		3.033772

				253.71		3.018161

				253.73		2.908883

				253.75		2.867253

				253.77		2.804808

				253.79		2.768382

				253.82		2.69553

				253.84		2.700734

				253.86		2.633085

				253.88		2.586252

				253.9		2.534214

				253.92		2.492585

				253.94		2.404121

				253.96		2.34688

				253.98		2.320862

				254		2.263621

				254.02		2.211583

				254.05		2.201176

				254.07		2.185565

				254.09		2.117916

				254.11		2.107509

				254.13		2.071083

				254.15		2.039861

				254.17		1.998231

				254.19		1.98262

				254.21		1.946193

				254.23		1.914971

				254.26		1.873341

				254.28		1.842119

				254.3		1.784878

				254.32		1.738044

				254.34		1.701618

				254.36		1.727637

				254.38		1.743248

				254.4		1.691211

				254.42		1.722433

				254.44		1.644377

				254.46		1.618359

				254.49		1.555914

				254.51		1.597544

				254.53		1.540303

				254.55		1.628766

				254.57		1.571525

				254.59		1.555914

				254.61		1.535099

				254.63		1.540303

				254.65		1.477858

				254.67		1.467451

				254.7		1.457043

				254.72		1.462247

				254.74		1.425821

				254.76		1.436228

				254.78		1.431025

				254.8		1.41021

				254.82		1.394599

				254.84		1.41021

				254.86		1.41021

				254.88		1.384191

				254.9		1.394599

				254.93		1.384191

				254.95		1.389395

				254.97		1.373784

				254.99		1.363376

				255.01		1.352969

				255.03		1.347765

				255.05		1.342561

				255.07		1.342561

				255.09		1.352969

				255.11		1.337358

				255.13		1.337358

				255.16		1.337358

				255.18		1.332154

				255.2		1.342561

				255.22		1.321746

				255.24		1.321746

				255.26		1.321746

				255.28		1.311339

				255.3		1.311339

				255.32		1.316543

				255.34		1.306135

				255.36		1.306135

				255.39		1.300931

				255.41		1.300931

				255.43		1.300931

				255.45		1.295728

				255.47		1.295728

				255.49		1.295728

				255.51		1.295728

				255.53		1.295728

				255.55		1.290524

				255.57		1.290524

				255.6		1.290524

				255.62		1.28532

				255.64		1.28532

				255.66		1.280117

				255.68		1.280117

				255.7		1.274913

				255.72		1.274913

				255.74		1.274913

				255.76		1.269709

				255.78		1.269709

				255.8		1.269709

				255.83		1.269709

				255.85		1.269709

				255.87		1.264505

				255.89		1.264505

				255.91		1.259302

				255.93		1.259302

				255.95		1.259302

				255.97		1.254098

				255.99		1.254098

				256.01		1.248894

				256.03		1.254098

				256.06		1.248894

				256.08		1.248894

				256.1		1.248894

				256.12		1.248894

				256.14		1.248894

				256.16		1.24369

				256.18		1.24369

				256.2		1.238487

				256.22		1.238487

				256.24		1.238487

				256.26		1.238487

				256.29		1.238487

				256.31		1.233283

				256.33		1.233283

				256.35		1.233283

				256.37		1.233283

				256.39		1.228079

				256.41		1.228079

				256.43		1.228079

				256.45		1.228079

				256.47		1.228079

				256.49		1.228079

				256.52		1.228079

				256.54		1.222876

				256.56		1.222876

				256.58		1.222876

				256.6		1.222876

				256.62		1.222876

				256.64		1.222876

				256.66		1.217672

				256.68		1.217672

				256.7		1.217672

				256.72		1.217672

				256.75		1.212468

				256.77		1.212468

				256.79		1.212468

				256.81		1.212468

				256.83		1.207264

				256.85		1.207264

				256.87		1.207264

				256.89		1.207264

				256.91		1.207264

				256.93		1.207264

				256.95		1.207264

				256.98		1.207264

				257		1.207264

				257.02		1.207264

				257.04		1.202061

				257.06		1.202061

				257.08		1.202061

				257.1		1.202061

				257.12		1.202061

				257.14		1.202061

				257.16		1.196857

				257.18		1.196857

				257.21		1.196857

				257.23		1.196857

				257.25		1.191653

				257.27		1.191653

				257.29		1.191653

				257.31		1.191653

				257.33		1.191653

				257.35		1.191653

				257.37		1.191653

				257.39		1.191653

				257.41		1.186449

				257.44		1.186449

				257.46		1.186449

				257.48		1.186449

				257.5		1.181246

				257.52		1.181246

				257.54		1.181246

				257.56		1.181246

				257.58		1.181246

				257.6		1.181246

				257.62		1.181246

				257.64		1.181246

				257.66		1.181246

				257.69		1.176042

				257.71		1.176042

				257.73		1.176042

				257.75		1.176042

				257.77		1.176042

				257.79		1.176042

				257.81		1.176042

				257.83		1.176042

				257.85		1.176042

				257.87		1.176042

				257.89		1.176042

				257.91		1.176042

				257.94		1.170838

				257.96		1.170838

				257.98		1.170838

				258		1.170838

				258.02		1.170838

				258.04		1.170838

				258.06		1.170838

				258.08		1.170838

				258.1		1.170838

				258.12		1.170838

				258.14		1.170838

				258.17		1.165635

				258.19		1.170838

				258.21		1.165635

				258.23		1.165635

				258.25		1.165635

				258.27		1.165635

				258.29		1.165635

				258.31		1.165635

				258.33		1.165635

				258.35		1.165635

				258.37		1.165635

				258.4		1.165635

				258.42		1.165635

				258.44		1.165635

				258.46		1.165635

				258.48		1.165635

				258.5		1.160431

				258.52		1.160431

				258.54		1.160431

				258.56		1.160431

				258.58		1.160431

				258.6		1.160431

				258.62		1.160431

				258.65		1.160431

				258.67		1.160431

				258.69		1.160431

				258.71		1.155227

				258.73		1.155227

				258.75		1.155227

				258.77		1.155227

				258.79		1.155227

				258.81		1.155227

				258.83		1.155227

				258.85		1.155227

				258.88		1.155227

				258.9		1.155227

				258.92		1.155227

				258.94		1.155227

				258.96		1.155227

				258.98		1.155227

				259		1.150023

				259.02		1.150023

				259.04		1.150023

				259.06		1.150023

				259.08		1.150023

				259.11		1.150023

				259.13		1.150023

				259.15		1.150023

				259.17		1.150023

				259.19		1.150023

				259.21		1.150023

				259.23		1.150023

				259.25		1.150023

				259.27		1.14482

				259.29		1.14482

				259.31		1.150023

				259.33		1.14482

				259.36		1.14482

				259.38		1.14482

				259.4		1.14482

				259.42		1.14482

				259.44		1.14482

				259.46		1.14482

				259.48		1.14482

				259.5		1.14482

				259.52		1.14482

				259.54		1.139616

				259.56		1.14482

				259.59		1.139616

				259.61		1.14482

				259.63		1.14482

				259.65		1.139616

				259.67		1.139616

				259.69		1.139616

				259.71		1.139616

				259.73		1.139616

				259.75		1.139616

				259.77		1.134412

				259.79		1.134412

				259.82		1.134412

				259.84		1.139616

				259.86		1.134412

				259.88		1.139616

				259.9		1.134412

				259.92		1.139616

				259.94		1.134412

				259.96		1.134412

				259.98		1.134412

				260		1.134412

				260.02		1.134412

				260.04		1.134412

				260.07		1.134412

				260.09		1.134412

				260.11		1.134412

				260.13		1.134412

				260.15		1.134412

				260.17		1.129209

				260.19		1.129209

				260.21		1.129209

				260.23		1.129209

				260.25		1.129209

				260.27		1.129209

				260.29		1.129209

				260.32		1.129209

				260.34		1.129209

				260.36		1.129209

				260.38		1.129209

				260.4		1.129209

				260.42		1.129209

				260.44		1.124005

				260.46		1.129209

				260.48		1.124005

				260.5		1.124005

				260.52		1.124005

				260.55		1.124005

				260.57		1.124005

				260.59		1.124005

				260.61		1.124005

				260.63		1.124005

				260.65		1.124005

				260.67		1.124005

				260.69		1.124005

				260.71		1.124005

				260.73		1.124005

				260.75		1.124005

				260.77		1.124005

				260.8		1.124005

				260.82		1.124005

				260.84		1.124005

				260.86		1.118801

				260.88		1.124005

				260.9		1.118801

				260.92		1.118801

				260.94		1.118801

				260.96		1.118801

				260.98		1.118801

				261		1.118801

				261.02		1.118801

				261.05		1.118801

				261.07		1.118801

				261.09		1.118801

				261.11		1.118801

				261.13		1.118801

				261.15		1.118801

				261.17		1.118801

				261.19		1.118801

				261.21		1.118801

				261.23		1.118801

				261.25		1.118801

				261.27		1.118801

				261.29		1.118801

				261.32		1.118801

				261.34		1.118801

				261.36		1.118801

				261.38		1.118801

				261.4		1.118801

				261.42		1.118801

				261.44		1.113597

				261.46		1.113597

				261.48		1.113597

				261.5		1.113597

				261.52		1.113597

				261.54		1.113597

				261.57		1.113597

				261.59		1.113597

				261.61		1.113597

				261.63		1.113597

				261.65		1.113597

				261.67		1.113597

				261.69		1.113597

				261.71		1.113597

				261.73		1.113597

				261.75		1.113597

				261.77		1.113597

				261.79		1.113597

				261.81		1.113597

				261.84		1.113597

				261.86		1.108394

				261.88		1.108394

				261.9		1.108394

				261.92		1.108394

				261.94		1.108394

				261.96		1.108394

				261.98		1.108394

				262		1.108394

				262.02		1.108394

				262.04		1.108394

				262.06		1.10319

				262.09		1.10319

				262.11		1.10319

				262.13		1.10319

				262.15		1.10319

				262.17		1.10319

				262.19		1.10319

				262.21		1.10319

				262.23		1.10319

				262.25		1.10319

				262.27		1.10319

				262.29		1.10319

				262.31		1.10319

				262.33		1.10319

				262.36		1.097986

				262.38		1.10319

				262.4		1.097986

				262.42		1.097986

				262.44		1.097986

				262.46		1.097986

				262.48		1.097986

				262.5		1.097986

				262.52		1.097986

				262.54		1.097986

				262.56		1.097986

				262.58		1.097986

				262.61		1.092782

				262.63		1.092782

				262.65		1.092782

				262.67		1.092782

				262.69		1.092782

				262.71		1.092782

				262.73		1.092782

				262.75		1.092782

				262.77		1.092782

				262.79		1.092782

				262.81		1.092782

				262.83		1.092782

				262.86		1.092782

				262.88		1.092782

				262.9		1.092782

				262.92		1.087579

				262.94		1.087579

				262.96		1.087579

				262.98		1.087579

				263		1.087579

				263.02		1.087579

				263.04		1.087579

				263.06		1.087579

				263.08		1.087579

				263.11		1.087579

				263.13		1.087579

				263.15		1.087579

				263.17		1.087579

				263.19		1.087579

				263.21		1.087579

				263.23		1.087579

				263.25		1.087579

				263.27		1.082375

				263.29		1.082375

				263.31		1.082375

				263.33		1.082375

				263.35		1.082375

				263.38		1.082375

				263.4		1.082375

				263.42		1.082375

				263.44		1.082375

				263.46		1.082375

				263.48		1.077171

				263.5		1.077171

				263.52		1.077171

				263.54		1.077171

				263.56		1.077171

				263.58		1.077171

				263.6		1.077171

				263.63		1.077171

				263.65		1.077171

				263.67		1.077171

				263.69		1.077171

				263.71		1.077171

				263.73		1.077171

				263.75		1.077171

				263.77		1.077171

				263.79		1.077171

				263.81		1.071968

				263.83		1.071968

				263.85		1.071968

				263.88		1.071968

				263.9		1.071968

				263.92		1.071968

				263.94		1.071968

				263.96		1.071968

				263.98		1.071968

				264		1.071968

				264.02		1.071968

				264.04		1.071968

				264.06		1.071968

				264.08		1.071968

				264.1		1.071968

				264.13		1.071968

				264.15		1.071968

				264.17		1.071968

				264.19		1.071968

				264.21		1.071968

				264.23		1.066764

				264.25		1.066764

				264.27		1.066764

				264.29		1.066764

				264.31		1.066764

				264.33		1.066764

				264.35		1.066764

				264.38		1.066764

				264.4		1.066764

				264.42		1.066764

				264.44		1.066764

				264.46		1.066764

				264.48		1.066764

				264.5		1.066764

				264.52		1.066764

				264.54		1.066764

				264.56		1.06156

				264.58		1.066764

				264.6		1.06156

				264.63		1.06156

				264.65		1.06156

				264.67		1.06156

				264.69		1.06156

				264.71		1.06156

				264.73		1.06156

				264.75		1.06156

				264.77		1.06156

				264.79		1.06156

				264.81		1.06156

				264.83		1.056356

				264.85		1.06156

				264.88		1.056356

				264.9		1.056356

				264.92		1.056356

				264.94		1.056356

				264.96		1.056356

				264.98		1.056356

				265		1.056356

				265.02		1.056356

				265.04		1.056356

				265.06		1.056356

				265.08		1.056356

				265.1		1.056356

				265.13		1.056356

				265.15		1.056356

				265.17		1.056356

				265.19		1.056356

				265.21		1.056356

				265.23		1.056356

				265.25		1.056356

				265.27		1.056356

				265.29		1.056356

				265.31		1.051153

				265.33		1.051153

				265.35		1.051153

				265.38		1.051153

				265.4		1.051153

				265.42		1.051153

				265.44		1.051153

				265.46		1.051153

				265.48		1.051153

				265.5		1.051153

				265.52		1.051153

				265.54		1.051153

				265.56		1.051153

				265.58		1.051153

				265.61		1.051153

				265.63		1.051153

				265.65		1.051153

				265.67		1.051153

				265.69		1.051153

				265.71		1.051153

				265.73		1.045949

				265.75		1.045949

				265.77		1.045949

				265.79		1.045949

				265.81		1.045949

				265.83		1.045949

				265.86		1.045949

				265.88		1.045949

				265.9		1.045949

				265.92		1.045949

				265.94		1.045949

				265.96		1.045949

				265.98		1.045949

				266		1.045949

				266.02		1.045949

				266.04		1.045949

				266.06		1.045949

				266.09		1.045949

				266.11		1.045949

				266.13		1.045949

				266.15		1.045949

				266.17		1.045949

				266.19		1.045949

				266.21		1.045949

				266.23		1.045949

				266.25		1.045949

				266.27		1.045949

				266.29		1.045949

				266.32		1.045949

				266.34		1.045949

				266.36		1.045949

				266.38		1.045949

				266.4		1.045949

				266.42		1.045949

				266.44		1.040745

				266.46		1.045949

				266.48		1.045949

				266.5		1.045949

				266.52		1.045949

				266.54		1.045949

				266.57		1.040745

				266.59		1.045949

				266.61		1.045949

				266.63		1.045949

				266.65		1.045949

				266.67		1.040745

				266.69		1.040745

				266.71		1.040745

				266.73		1.040745

				266.75		1.040745

				266.77		1.040745

				266.8		1.040745

				266.82		1.040745

				266.84		1.040745

				266.86		1.040745

				266.88		1.040745

				266.9		1.040745

				266.92		1.040745

				266.94		1.040745

				266.96		1.040745

				266.98		1.040745

				267		1.040745

				267.03		1.040745

				267.05		1.040745

				267.07		1.040745

				267.09		1.040745

				267.11		1.040745

				267.13		1.040745

				267.15		1.040745

				267.17		1.040745

				267.19		1.040745

				267.21		1.040745

				267.23		1.040745

				267.25		1.040745

				267.28		1.035541

				267.3		1.035541

				267.32		1.035541

				267.34		1.035541

				267.36		1.035541

				267.38		1.035541

				267.4		1.035541

				267.42		1.035541

				267.44		1.040745

				267.46		1.040745

				267.48		1.040745

				267.51		1.035541

				267.53		1.040745

				267.55		1.040745

				267.57		1.035541

				267.59		1.035541

				267.61		1.035541

				267.63		1.035541

				267.65		1.035541

				267.67		1.035541

				267.69		1.035541

				267.71		1.035541

				267.74		1.035541

				267.76		1.035541

				267.78		1.035541

				267.8		1.035541

				267.82		1.035541

				267.84		1.035541

				267.86		1.035541

				267.88		1.035541

				267.9		1.035541

				267.92		1.030338

				267.94		1.030338

				267.96		1.030338

				267.99		1.030338

				268.01		1.030338

				268.03		1.030338

				268.05		1.030338

				268.07		1.030338

				268.09		1.030338

				268.11		1.030338

				268.13		1.030338

				268.15		1.030338

				268.17		1.030338

				268.19		1.025134

				268.22		1.025134

				268.24		1.025134

				268.26		1.025134

				268.28		1.025134

				268.3		1.025134

				268.32		1.025134

				268.34		1.025134

				268.36		1.01993

				268.38		1.025134

				268.4		1.01993

				268.42		1.01993

				268.45		1.01993

				268.47		1.01993

				268.49		1.01993

				268.51		1.01993

				268.53		1.01993

				268.55		1.01993

				268.57		1.01993

				268.59		1.01993

				268.61		1.01993

				268.63		1.014727

				268.65		1.014727

				268.67		1.014727

				268.7		1.014727

				268.72		1.014727

				268.74		1.014727

				268.76		1.014727

				268.78		1.014727

				268.8		1.014727

				268.82		1.014727

				268.84		1.014727

				268.86		1.009523

				268.88		1.009523

				268.91		1.009523

				268.93		1.009523

				268.95		1.009523

				268.97		1.009523

				268.99		1.009523

				269.01		1.009523

				269.03		1.009523

				269.05		1.009523

				269.07		1.009523

				269.09		1.009523

				269.11		1.009523

				269.13		1.009523

				269.16		1.009523

				269.18		1.009523

				269.2		1.009523

				269.22		1.009523

				269.24		1.004319

				269.26		1.004319

				269.28		1.004319

				269.3		1.004319

				269.32		1.004319

				269.34		1.004319

				269.36		1.004319

				269.39		1.004319

				269.41		1.004319

				269.43		1.004319

				269.45		1.004319

				269.47		0.9991154

				269.49		1.004319

				269.51		0.9991154

				269.53		0.9991154

				269.55		0.9991154

				269.57		0.9991154

				269.59		0.9991154

				269.62		0.9991154

				269.64		0.9991154

				269.66		0.9939116

				269.68		0.9939116

				269.7		0.9939116

				269.72		0.9939116

				269.74		0.9939116

				269.76		0.9939116

				269.78		0.9939116

				269.8		0.9939116

				269.82		0.9939116

				269.85		0.9887079

				269.87		0.9939116

				269.89		0.9887079

				269.91		0.9887079

				269.93		0.9887079

				269.95		0.9887079

				269.97		0.9887079

				269.99		0.9887079

				270.01		0.9887079

				270.03		0.9887079

				270.05		0.9887079

				270.08		0.9887079

				270.1		0.9887079

				270.12		0.9887079

				270.14		0.9887079

				270.16		0.9887079

				270.18		0.9887079

				270.2		0.9887079

				270.22		0.9887079

				270.24		0.9887079

				270.26		0.9887079

				270.28		0.9887079

				270.31		0.9887079

				270.33		0.9887079

				270.35		0.9887079

				270.37		0.9887079

				270.39		0.9887079

				270.41		0.9887079

				270.43		0.9887079

				270.45		0.9835042

				270.47		0.9887079

				270.49		0.9835042

				270.51		0.9835042

				270.54		0.9835042

				270.56		0.9835042

				270.58		0.9835042

				270.6		0.9835042

				270.62		0.9835042

				270.64		0.9835042

				270.66		0.9835042

				270.68		0.9835042

				270.7		0.9835042

				270.72		0.9835042

				270.74		0.9835042

				270.77		0.9835042

				270.79		0.9835042

				270.81		0.9835042

				270.83		0.9783005

				270.85		0.9835042

				270.87		0.9783005

				270.89		0.9783005

				270.91		0.9783005

				270.93		0.9783005

				270.95		0.9783005

				270.98		0.9783005

				271		0.9783005

				271.02		0.9783005

				271.04		0.9783005

				271.06		0.9783005

				271.08		0.9783005

				271.1		0.9783005

				271.12		0.9783005

				271.14		0.9783005

				271.16		0.9783005

				271.18		0.9783005

				271.21		0.9783005

				271.23		0.9783005

				271.25		0.9783005

				271.27		0.9783005

				271.29		0.9783005

				271.31		0.9783005

				271.33		0.9783005

				271.35		0.9783005

				271.37		0.9783005

				271.39		0.9783005

				271.41		0.9783005

				271.44		0.9783005

				271.46		0.9783005

				271.48		0.9783005

				271.5		0.9783005

				271.52		0.9783005

				271.54		0.9783005

				271.56		0.9783005

				271.58		0.9783005

				271.6		0.9783005

				271.62		0.9783005

				271.64		0.9783005

				271.67		0.9783005

				271.69		0.9730967

				271.71		0.9730967

				271.73		0.9730967

				271.75		0.9730967

				271.77		0.9730967

				271.79		0.9730967

				271.81		0.9730967

				271.83		0.9730967

				271.85		0.9730967

				271.88		0.9730967

				271.9		0.9730967

				271.92		0.9730967

				271.94		0.9730967

				271.96		0.9730967

				271.98		0.9730967

				272		0.9730967

				272.02		0.9730967

				272.04		0.9730967

				272.06		0.9730967

				272.08		0.9730967

				272.11		0.9730967

				272.13		0.9730967

				272.15		0.9730967

				272.17		0.9730967

				272.19		0.9730967

				272.21		0.9730967

				272.23		0.9730967

				272.25		0.9730967

				272.27		0.9730967

				272.29		0.9730967

				272.31		0.9730967

				272.34		0.967893

				272.36		0.9730967

				272.38		0.9730967

				272.4		0.9730967

				272.42		0.967893

				272.44		0.967893

				272.46		0.967893

				272.48		0.967893

				272.5		0.967893

				272.52		0.967893

				272.55		0.967893

				272.57		0.967893

				272.59		0.967893

				272.61		0.967893

				272.63		0.967893

				272.65		0.967893

				272.67		0.967893

				272.69		0.967893

				272.71		0.967893

				272.73		0.967893

				272.75		0.967893

				272.78		0.967893

				272.8		0.967893

				272.82		0.967893

				272.84		0.967893

				272.86		0.967893

				272.88		0.967893

				272.9		0.967893

				272.92		0.967893

				272.94		0.967893

				272.96		0.967893

				272.99		0.967893

				273.01		0.967893

				273.03		0.967893

				273.05		0.967893

				273.07		0.9626893

				273.09		0.9626893

				273.11		0.9626893

				273.13		0.9626893

				273.15		0.9626893

				273.17		0.9626893

				273.19		0.9626893

				273.22		0.9626893

				273.24		0.9626893

				273.26		0.9626893

				273.28		0.9626893

				273.3		0.9626893

				273.32		0.9626893

				273.34		0.9626893

				273.36		0.9574856

				273.38		0.9574856

				273.4		0.9574856

				273.43		0.9574856

				273.45		0.9574856

				273.47		0.9574856

				273.49		0.9574856

				273.51		0.9574856

				273.53		0.9574856

				273.55		0.9574856

				273.57		0.9574856

				273.59		0.9574856

				273.61		0.9574856

				273.63		0.9574856

				273.66		0.9574856

				273.68		0.9574856

				273.7		0.9574856

				273.72		0.9574856

				273.74		0.9574856

				273.76		0.9574856

				273.78		0.9574856

				273.8		0.9574856

				273.82		0.9574856

				273.84		0.9574856

				273.87		0.9574856

				273.89		0.9574856

				273.91		0.9574856

				273.93		0.9574856

				273.95		0.9574856

				273.97		0.9574856

				273.99		0.9574856

				274.01		0.9522818

				274.03		0.9574856

				274.05		0.9522818

				274.07		0.9522818

				274.1		0.9522818

				274.12		0.9522818

				274.14		0.9522818

				274.16		0.9522818

				274.18		0.9522818

				274.2		0.9522818

				274.22		0.9522818

				274.24		0.9522818

				274.26		0.9522818

				274.28		0.9522818

				274.31		0.9522818

				274.33		0.9522818

				274.35		0.9522818

				274.37		0.9522818

				274.39		0.9522818

				274.41		0.9522818

				274.43		0.9522818

				274.45		0.9522818

				274.47		0.9522818

				274.49		0.9522818

				274.51		0.9522818

				274.54		0.9522818

				274.56		0.9522818

				274.58		0.9522818

				274.6		0.9522818

				274.62		0.9522818

				274.64		0.9522818

				274.66		0.9522818

				274.68		0.9522818

				274.7		0.9522818

				274.72		0.9522818

				274.75		0.9470781

				274.77		0.9470781

				274.79		0.9522818

				274.81		0.9470781

				274.83		0.9470781

				274.85		0.9470781

				274.87		0.9470781

				274.89		0.9470781

				274.91		0.9470781

				274.93		0.9470781

				274.95		0.9470781

				274.98		0.9470781

				275		0.9470781

				275.02		0.9470781

				275.04		0.9470781

				275.06		0.9470781

				275.08		0.9470781

				275.1		0.9418744

				275.12		0.9418744

				275.14		0.9418744

				275.16		0.9418744

				275.19		0.9418744

				275.21		0.9418744

				275.23		0.9418744

				275.25		0.9418744

				275.27		0.9418744

				275.29		0.9418744

				275.31		0.9418744

				275.33		0.9418744

				275.35		0.9418744

				275.37		0.9418744

				275.39		0.9418744

				275.42		0.9418744

				275.44		0.9418744

				275.46		0.9418744

				275.48		0.9418744

				275.5		0.9418744

				275.52		0.9418744

				275.54		0.9418744

				275.56		0.9418744

				275.58		0.9418744

				275.6		0.9418744

				275.62		0.9418744

				275.65		0.9418744

				275.67		0.9418744

				275.69		0.9418744

				275.71		0.9418744

				275.73		0.9418744

				275.75		0.9418744

				275.77		0.9418744

				275.79		0.9418744

				275.81		0.9418744

				275.83		0.9418744

				275.86		0.9366707

				275.88		0.9366707

				275.9		0.9366707

				275.92		0.9366707

				275.94		0.9366707

				275.96		0.9366707

				275.98		0.9366707

				276		0.9366707

				276.02		0.9366707

				276.04		0.9366707

				276.06		0.9366707

				276.09		0.9366707

				276.11		0.9366707

				276.13		0.9366707

				276.15		0.9366707

				276.17		0.9366707

				276.19		0.9366707

				276.21		0.9366707

				276.23		0.9366707

				276.25		0.9366707

				276.27		0.9366707

				276.29		0.9366707

				276.32		0.9366707

				276.34		0.9366707

				276.36		0.9366707

				276.38		0.9366707

				276.4		0.9366707

				276.42		0.9366707

				276.44		0.9366707

				276.46		0.9366707

				276.48		0.9366707

				276.5		0.9366707

				276.53		0.9366707

				276.55		0.9366707

				276.57		0.9366707

				276.59		0.9366707

				276.61		0.9366707

				276.63		0.9366707

				276.65		0.9366707

				276.67		0.9366707

				276.69		0.9366707

				276.71		0.9366707

				276.73		0.9366707

				276.76		0.9366707

				276.78		0.9366707

				276.8		0.9366707

				276.82		0.9366707

				276.84		0.9366707

				276.86		0.9366707

				276.88		0.9366707

				276.9		0.9366707

				276.92		0.9366707

				276.94		0.9366707

				276.97		0.9366707

				276.99		0.9366707

				277.01		0.9418744

				277.03		0.9366707

				277.05		0.9418744

				277.07		0.9418744

				277.09		0.9418744

				277.11		0.9418744

				277.13		0.9418744

				277.15		0.9418744

				277.17		0.9418744

				277.2		0.9418744

				277.22		0.9418744

				277.24		0.9418744

				277.26		0.9418744

				277.28		0.9418744

				277.3		0.9470781

				277.32		0.9470781

				277.34		0.9470781

				277.36		0.9470781

				277.38		0.9470781

				277.41		0.9470781

				277.43		0.9470781

				277.45		0.9470781

				277.47		0.9470781

				277.49		0.9470781

				277.51		0.9470781

				277.53		0.9470781

				277.55		0.9470781

				277.57		0.9470781

				277.59		0.9470781

				277.61		0.9470781

				277.64		0.9470781

				277.66		0.9470781

				277.68		0.9470781

				277.7		0.9470781

				277.72		0.9470781

				277.74		0.9470781

				277.76		0.9470781

				277.78		0.9470781

				277.8		0.9470781

				277.82		0.9470781

				277.84		0.9470781

				277.87		0.9470781

				277.89		0.9470781

				277.91		0.9470781

				277.93		0.9470781

				277.95		0.9470781

				277.97		0.9470781

				277.99		0.9470781

				278.01		0.9470781

				278.03		0.9470781

				278.05		0.9470781

				278.08		0.9470781

				278.1		0.9470781

				278.12		0.9470781

				278.14		0.9470781

				278.16		0.9470781

				278.18		0.9470781

				278.2		0.9470781

				278.22		0.9470781

				278.24		0.9470781

				278.26		0.9470781

				278.28		0.9470781

				278.31		0.9470781

				278.33		0.9470781

				278.35		0.9470781

				278.37		0.9470781

				278.39		0.9470781

				278.41		0.9470781

				278.43		0.9470781

				278.45		0.9470781

				278.47		0.9470781

				278.49		0.9470781

				278.51		0.9470781

				278.54		0.9470781

				278.56		0.9470781

				278.58		0.9470781

				278.6		0.9470781

				278.62		0.9470781

				278.64		0.9470781

				278.66		0.9470781

				278.68		0.9470781

				278.7		0.9470781

				278.72		0.9470781

				278.75		0.9470781

				278.77		0.9470781

				278.79		0.9470781

				278.81		0.9470781

				278.83		0.9418744

				278.85		0.9418744

				278.87		0.9470781

				278.89		0.9418744

				278.91		0.9470781

				278.93		0.9418744

				278.95		0.9418744

				278.98		0.9418744

				279		0.9418744

				279.02		0.9418744

				279.04		0.9418744

				279.06		0.9418744

				279.08		0.9418744

				279.1		0.9418744

				279.12		0.9418744

				279.14		0.9418744

				279.16		0.9418744

				279.18		0.9418744

				279.21		0.9418744

				279.23		0.9418744

				279.25		0.9418744

				279.27		0.9418744

				279.29		0.9418744

				279.31		0.9366707

				279.33		0.9366707

				279.35		0.9366707

				279.37		0.9366707

				279.39		0.9366707

				279.41		0.9366707

				279.44		0.9366707

				279.46		0.9366707

				279.48		0.9366707

				279.5		0.9366707

				279.52		0.9366707

				279.54		0.9366707

				279.56		0.9366707

				279.58		0.9366707

				279.6		0.9366707

				279.62		0.9366707

				279.64		0.9314669

				279.67		0.9314669

				279.69		0.9314669

				279.71		0.9366707

				279.73		0.9314669

				279.75		0.9314669

				279.77		0.9314669

				279.79		0.9314669

				279.81		0.9314669

				279.83		0.9314669

				279.85		0.9314669

				279.87		0.9314669

				279.9		0.9314669

				279.92		0.9314669

				279.94		0.9314669

				279.96		0.9314669

				279.98		0.9314669

				280		0.9314669

				280.02		0.9314669

				280.04		0.9314669

				280.06		0.9314669

				280.08		0.9314669

				280.11		0.9314669

				280.13		0.9314669

				280.15		0.9314669

				280.17		0.9314669

				280.19		0.9314669

				280.21		0.9314669

				280.23		0.9314669

				280.25		0.9262632

				280.27		0.9262632

				280.29		0.9262632

				280.31		0.9262632

				280.34		0.9262632

				280.36		0.9262632

				280.38		0.9262632

				280.4		0.9262632

				280.42		0.9262632

				280.44		0.9262632

				280.46		0.9262632

				280.48		0.9262632

				280.5		0.9262632

				280.52		0.9262632

				280.55		0.9314669

				280.57		0.9262632

				280.59		0.9262632

				280.61		0.9262632

				280.63		0.9262632

				280.65		0.9262632

				280.67		0.9262632

				280.69		0.9262632

				280.71		0.9262632

				280.73		0.9262632

				280.75		0.9262632

				280.78		0.9262632

				280.8		0.9262632

				280.82		0.9262632

				280.84		0.9262632

				280.86		0.9262632

				280.88		0.9262632

				280.9		0.9262632

				280.92		0.9262632

				280.94		0.9262632

				280.96		0.9262632

				280.99		0.9262632

				281.01		0.9262632

				281.03		0.9262632

				281.05		0.9262632

				281.07		0.9262632

				281.09		0.9262632

				281.11		0.9262632

				281.13		0.9262632

				281.15		0.9262632

				281.17		0.9262632

				281.19		0.9262632

				281.22		0.9262632

				281.24		0.9262632

				281.26		0.9262632

				281.28		0.9210595

				281.3		0.9210595

				281.32		0.9210595

				281.34		0.9210595

				281.36		0.9210595

				281.38		0.9262632

				281.4		0.9210595

				281.43		0.9210595

				281.45		0.9210595

				281.47		0.9210595

				281.49		0.9210595

				281.51		0.9210595

				281.53		0.9210595

				281.55		0.9262632

				281.57		0.9262632

				281.59		0.9262632

				281.61		0.9262632

				281.63		0.9262632

				281.66		0.9262632

				281.68		0.9262632

				281.7		0.9262632

				281.72		0.9210595

				281.74		0.9210595

				281.76		0.9210595

				281.78		0.9210595

				281.8		0.9210595

				281.82		0.9210595

				281.84		0.9210595

				281.87		0.9210595

				281.89		0.9210595

				281.91		0.9210595

				281.93		0.9210595

				281.95		0.9210595

				281.97		0.9210595

				281.99		0.9210595

				282.01		0.9210595

				282.03		0.9210595

				282.05		0.9210595

				282.07		0.9210595

				282.1		0.9210595

				282.12		0.9210595

				282.14		0.9210595

				282.16		0.9210595

				282.18		0.9210595

				282.2		0.9210595

				282.22		0.9210595

				282.24		0.9210595

				282.26		0.9210595

				282.28		0.9210595

				282.31		0.9210595

				282.33		0.9210595

				282.35		0.9210595

				282.37		0.9210595

				282.39		0.9262632

				282.41		0.9262632

				282.43		0.9210595

				282.45		0.9210595

				282.47		0.9210595

				282.49		0.9210595

				282.52		0.9262632

				282.54		0.9210595

				282.56		0.9210595

				282.58		0.9210595

				282.6		0.9210595

				282.62		0.9210595

				282.64		0.9210595

				282.66		0.9210595

				282.68		0.9210595

				282.7		0.9210595

				282.72		0.9210595

				282.75		0.9210595

				282.77		0.9210595

				282.79		0.9210595

				282.81		0.9210595

				282.83		0.9210595

				282.85		0.9210595

				282.87		0.9158558

				282.89		0.9210595

				282.91		0.9210595

				282.93		0.9158558

				282.95		0.9158558

				282.98		0.9158558

				283		0.9158558

				283.02		0.9158558

				283.04		0.9158558

				283.06		0.9158558

				283.08		0.9158558

				283.1		0.9158558

				283.12		0.9158558

				283.14		0.9158558

				283.16		0.9158558

				283.19		0.9158558

				283.21		0.9158558

				283.23		0.9158558

				283.25		0.9158558

				283.27		0.9158558

				283.29		0.9158558

				283.31		0.9158558

				283.33		0.9158558

				283.35		0.9158558

				283.37		0.9158558

				283.39		0.9158558

				283.42		0.9158558

				283.44		0.9158558

				283.46		0.9158558

				283.48		0.9158558

				283.5		0.9158558

				283.52		0.9158558

				283.54		0.9158558

				283.56		0.910652

				283.58		0.9158558

				283.6		0.910652

				283.63		0.910652

				283.65		0.910652

				283.67		0.910652

				283.69		0.910652

				283.71		0.910652

				283.73		0.910652

				283.75		0.910652

				283.77		0.910652

				283.79		0.910652

				283.81		0.910652

				283.83		0.910652

				283.86		0.910652

				283.88		0.910652

				283.9		0.910652

				283.92		0.910652

				283.94		0.910652

				283.96		0.910652

				283.98		0.910652

				284		0.910652

				284.02		0.910652

				284.04		0.910652

				284.07		0.910652

				284.09		0.910652

				284.11		0.910652

				284.13		0.910652

				284.15		0.910652

				284.17		0.910652

				284.19		0.910652

				284.21		0.910652

				284.23		0.9054483

				284.25		0.910652

				284.27		0.910652

				284.3		0.910652

				284.32		0.9054483

				284.34		0.910652

				284.36		0.9054483

				284.38		0.9054483

				284.4		0.9054483

				284.42		0.9054483

				284.44		0.9054483

				284.46		0.9054483

				284.48		0.9054483

				284.51		0.9054483

				284.53		0.910652

				284.55		0.910652

				284.57		0.910652

				284.59		0.9054483

				284.61		0.910652

				284.63		0.910652

				284.65		0.910652

				284.67		0.9054483

				284.69		0.9054483

				284.72		0.9054483

				284.74		0.9054483

				284.76		0.9054483

				284.78		0.9054483

				284.8		0.9054483

				284.82		0.9054483

				284.84		0.9054483

				284.86		0.9054483

				284.88		0.910652

				284.9		0.9054483

				284.92		0.910652

				284.95		0.910652

				284.97		0.910652

				284.99		0.910652

				285.01		0.910652

				285.03		0.910652

				285.05		0.910652

				285.07		0.910652

				285.09		0.910652

				285.11		0.910652

				285.13		0.910652

				285.16		0.910652

				285.18		0.910652

				285.2		0.9054483

				285.22		0.9054483

				285.24		0.9054483

				285.26		0.910652

				285.28		0.910652

				285.3		0.910652

				285.32		0.910652

				285.34		0.910652

				285.37		0.910652

				285.39		0.910652

				285.41		0.910652

				285.43		0.910652

				285.45		0.910652

				285.47		0.910652

				285.49		0.910652

				285.51		0.910652

				285.53		0.910652

				285.55		0.910652

				285.58		0.910652

				285.6		0.910652

				285.62		0.910652

				285.64		0.910652

				285.66		0.910652

				285.68		0.910652

				285.7		0.910652

				285.72		0.910652

				285.74		0.910652

				285.76		0.910652

				285.79		0.910652

				285.81		0.910652

				285.83		0.910652

				285.85		0.910652

				285.87		0.910652

				285.89		0.910652

				285.91		0.9158558

				285.93		0.9158558

				285.95		0.9158558

				285.97		0.910652

				285.99		0.910652

				286.02		0.910652

				286.04		0.910652

				286.06		0.9158558

				286.08		0.9158558

				286.1		0.910652

				286.12		0.9158558

				286.14		0.9158558

				286.16		0.910652

				286.18		0.9158558

				286.2		0.910652

				286.23		0.910652

				286.25		0.910652

				286.27		0.910652

				286.29		0.910652

				286.31		0.9158558

				286.33		0.910652

				286.35		0.9158558

				286.37		0.910652

				286.39		0.9158558

				286.41		0.910652

				286.44		0.910652

				286.46		0.9158558

				286.48		0.9158558

				286.5		0.910652

				286.52		0.910652

				286.54		0.910652

				286.56		0.910652

				286.58		0.910652

				286.6		0.910652

				286.62		0.910652

				286.65		0.910652

				286.67		0.910652

				286.69		0.910652

				286.71		0.910652

				286.73		0.910652

				286.75		0.910652

				286.77		0.910652

				286.79		0.910652

				286.81		0.910652

				286.83		0.910652

				286.86		0.910652

				286.88		0.910652

				286.9		0.910652

				286.92		0.910652

				286.94		0.910652

				286.96		0.910652

				286.98		0.910652

				287		0.910652

				287.02		0.910652

				287.04		0.910652

				287.07		0.910652

				287.09		0.910652

				287.11		0.910652

				287.13		0.910652

				287.15		0.910652

				287.17		0.910652

				287.19		0.910652

				287.21		0.910652

				287.23		0.910652

				287.25		0.910652

				287.27		0.910652

				287.3		0.910652

				287.32		0.910652

				287.34		0.910652

				287.36		0.910652

				287.38		0.910652

				287.4		0.910652

				287.42		0.910652

				287.44		0.910652

				287.46		0.910652

				287.48		0.910652

				287.51		0.910652

				287.53		0.910652

				287.55		0.910652

				287.57		0.910652

				287.59		0.9054483

				287.61		0.910652

				287.63		0.9054483

				287.65		0.9054483

				287.67		0.9054483

				287.69		0.9054483

				287.72		0.9054483

				287.74		0.9054483

				287.76		0.9054483

				287.78		0.9054483

				287.8		0.9054483

				287.82		0.9054483

				287.84		0.9054483

				287.86		0.9054483

				287.88		0.9054483

				287.9		0.9054483

				287.93		0.9054483

				287.95		0.9054483

				287.97		0.9054483

				287.99		0.9054483

				288.01		0.9054483

				288.03		0.9054483

				288.05		0.9054483

				288.07		0.9054483

				288.09		0.9002446

				288.11		0.9002446

				288.14		0.9054483

				288.16		0.9002446

				288.18		0.9002446

				288.2		0.9002446

				288.22		0.9002446

				288.24		0.9002446

				288.26		0.9002446

				288.28		0.9002446

				288.3		0.9002446

				288.32		0.9002446

				288.35		0.9002446

				288.37		0.9002446

				288.39		0.9002446

				288.41		0.9002446

				288.43		0.9002446

				288.45		0.9002446

				288.47		0.9002446

				288.49		0.9002446

				288.51		0.9002446

				288.53		0.9002446

				288.56		0.9002446

				288.58		0.9002446

				288.6		0.9002446

				288.62		0.9002446

				288.64		0.9002446

				288.66		0.9002446

				288.68		0.9002446

				288.7		0.9002446

				288.72		0.9002446

				288.74		0.9002446

				288.77		0.9002446

				288.79		0.9002446

				288.81		0.9002446

				288.83		0.9002446

				288.85		0.9002446

				288.87		0.9002446

				288.89		0.9002446

				288.91		0.9002446

				288.93		0.9002446

				288.95		0.8950408

				288.98		0.9002446

				289		0.8950408

				289.02		0.9002446

				289.04		0.8950408

				289.06		0.8950408

				289.08		0.8950408

				289.1		0.8950408

				289.12		0.8950408

				289.14		0.8950408

				289.16		0.8950408

				289.19		0.8950408

				289.21		0.8950408

				289.23		0.8950408

				289.25		0.8950408

				289.27		0.8950408

				289.29		0.8950408

				289.31		0.8950408

				289.33		0.8950408

				289.35		0.8950408

				289.37		0.8950408

				289.4		0.8950408

				289.42		0.8950408

				289.44		0.8950408

				289.46		0.8950408

				289.48		0.8950408

				289.5		0.8950408

				289.52		0.9002446

				289.54		0.8950408

				289.56		0.9002446

				289.58		0.9002446

				289.61		0.9002446

				289.63		0.9002446

				289.65		0.9002446

				289.67		0.9002446

				289.69		0.9002446

				289.71		0.9002446

				289.73		0.9002446

				289.75		0.9002446

				289.77		0.9002446

				289.79		0.9002446

				289.82		0.9002446

				289.84		0.9002446

				289.86		0.9054483

				289.88		0.9054483

				289.9		0.9054483

				289.92		0.9054483

				289.94		0.9054483

				289.96		0.9054483

				289.98		0.9002446

				290		0.9002446

				290.03		0.9002446

				290.05		0.9002446

				290.07		0.9002446

				290.09		0.9002446

				290.11		0.9002446

				290.13		0.9002446

				290.15		0.9054483

				290.17		0.9054483

				290.19		0.9054483

				290.22		0.9054483

				290.24		0.9054483

				290.26		0.9054483

				290.28		0.9054483

				290.3		0.9054483

				290.32		0.9054483

				290.34		0.9054483

				290.36		0.9054483

				290.38		0.9054483

				290.4		0.9054483

				290.43		0.9054483

				290.45		0.9054483

				290.47		0.9054483

				290.49		0.9054483

				290.51		0.9054483

				290.53		0.9054483

				290.55		0.9054483

				290.57		0.9054483

				290.59		0.9054483

				290.61		0.9054483

				290.64		0.9054483

				290.66		0.9054483

				290.68		0.9054483

				290.7		0.9054483

				290.72		0.9054483

				290.74		0.9054483

				290.76		0.9002446

				290.78		0.9054483

				290.8		0.9054483

				290.82		0.9054483

				290.85		0.9002446

				290.87		0.9054483

				290.89		0.9002446

				290.91		0.9002446

				290.93		0.9002446

				290.95		0.9002446

				290.97		0.9002446

				290.99		0.9002446

				291.01		0.9002446

				291.03		0.9002446

				291.06		0.9002446

				291.08		0.9002446

				291.1		0.9002446

				291.12		0.9002446

				291.14		0.9002446

				291.16		0.9002446

				291.18		0.9002446

				291.2		0.9002446

				291.22		0.9002446

				291.24		0.9002446

				291.27		0.9002446

				291.29		0.9002446

				291.31		0.9002446

				291.33		0.9002446

				291.35		0.9002446

				291.37		0.9002446

				291.39		0.9002446

				291.41		0.9002446

				291.43		0.8950408

				291.45		0.8950408

				291.48		0.8950408

				291.5		0.8950408

				291.52		0.8950408

				291.54		0.8950408

				291.56		0.8950408

				291.58		0.8950408

				291.6		0.8950408

				291.62		0.8950408

				291.64		0.8950408

				291.66		0.8950408

				291.69		0.8950408

				291.71		0.8950408

				291.73		0.8950408

				291.75		0.8950408

				291.77		0.8898371

				291.79		0.8898371

				291.81		0.8898371

				291.83		0.8898371

				291.85		0.8898371

				291.88		0.8898371

				291.9		0.8898371

				291.92		0.8898371

				291.94		0.8898371

				291.96		0.8898371

				291.98		0.8898371

				292		0.8898371

				292.02		0.8898371

				292.04		0.8898371

				292.06		0.8898371

				292.09		0.8898371

				292.11		0.8898371

				292.13		0.8898371

				292.15		0.8898371

				292.17		0.8898371

				292.19		0.8898371

				292.21		0.8846334

				292.23		0.8846334

				292.25		0.8846334

				292.27		0.8846334

				292.3		0.8846334

				292.32		0.8846334

				292.34		0.8846334

				292.36		0.8846334

				292.38		0.8846334

				292.4		0.8846334

				292.42		0.8846334

				292.44		0.8846334

				292.46		0.8846334

				292.48		0.8846334

				292.51		0.8794297

				292.53		0.8794297

				292.55		0.8846334

				292.57		0.8846334

				292.59		0.8846334

				292.61		0.8846334

				292.63		0.8846334

				292.65		0.8846334

				292.67		0.8846334

				292.69		0.8846334

				292.72		0.8846334

				292.74		0.8846334

				292.76		0.8846334

				292.78		0.8846334

				292.8		0.8846334

				292.82		0.8846334

				292.84		0.8846334

				292.86		0.8846334

				292.88		0.8846334

				292.91		0.8846334

				292.93		0.8846334

				292.95		0.8846334

				292.97		0.8846334

				292.99		0.8846334

				293.01		0.8846334

				293.03		0.8846334

				293.05		0.8846334

				293.07		0.8794297

				293.09		0.8846334

				293.12		0.8794297

				293.14		0.8846334

				293.16		0.8846334

				293.18		0.8846334

				293.2		0.8794297

				293.22		0.8846334

				293.24		0.8846334

				293.26		0.8846334

				293.28		0.8846334

				293.3		0.8846334

				293.33		0.8846334

				293.35		0.8846334

				293.37		0.8846334

				293.39		0.8846334

				293.41		0.8846334

				293.43		0.8846334

				293.45		0.8846334

				293.47		0.8846334

				293.49		0.8846334

				293.52		0.8846334

				293.54		0.8846334

				293.56		0.8846334

				293.58		0.8846334

				293.6		0.8846334

				293.62		0.8846334

				293.64		0.8846334

				293.66		0.8846334

				293.68		0.8846334

				293.7		0.8846334

				293.73		0.8846334

				293.75		0.8846334

				293.77		0.8846334

				293.79		0.8794297

				293.81		0.8846334

				293.83		0.8846334

				293.85		0.8846334

				293.87		0.8846334

				293.89		0.8794297

				293.91		0.8794297

				293.94		0.8846334

				293.96		0.8846334

				293.98		0.8794297

				294		0.8794297

				294.02		0.8794297

				294.04		0.8794297

				294.06		0.8794297

				294.08		0.8794297

				294.1		0.8794297

				294.13		0.8794297

				294.15		0.8794297

				294.17		0.8794297

				294.19		0.8794297

				294.21		0.8794297

				294.23		0.8794297

				294.25		0.8794297

				294.27		0.8794297

				294.29		0.8794297

				294.31		0.8794297

				294.34		0.8794297

				294.36		0.8794297

				294.38		0.8794297

				294.4		0.8742259

				294.42		0.8742259

				294.44		0.8742259

				294.46		0.8742259

				294.48		0.8742259

				294.5		0.8742259

				294.53		0.8742259

				294.55		0.8742259

				294.57		0.8742259

				294.59		0.8742259

				294.61		0.8742259

				294.63		0.8742259

				294.65		0.8742259

				294.67		0.8742259

				294.69		0.8742259

				294.71		0.8742259

				294.74		0.8742259

				294.76		0.8742259

				294.78		0.8742259

				294.8		0.8742259

				294.82		0.8742259

				294.84		0.8742259

				294.86		0.8742259

				294.88		0.8742259

				294.9		0.8690222

				294.93		0.8690222

				294.95		0.8690222

				294.97		0.8690222

				294.99		0.8690222

				295.01		0.8690222

				295.03		0.8690222

				295.05		0.8690222

				295.07		0.8690222

				295.09		0.8690222

				295.11		0.8690222

				295.14		0.8690222

				295.16		0.8690222

				295.18		0.8690222

				295.2		0.8690222

				295.22		0.8690222

				295.24		0.8690222

				295.26		0.8690222

				295.28		0.8690222

				295.3		0.8690222

				295.33		0.8690222

				295.35		0.8690222

				295.37		0.8690222

				295.39		0.8690222

				295.41		0.8690222

				295.43		0.8690222

				295.45		0.8690222

				295.47		0.8690222

				295.49		0.8690222

				295.51		0.8690222

				295.54		0.8690222

				295.56		0.8690222

				295.58		0.8690222

				295.6		0.8690222

				295.62		0.8690222

				295.64		0.8690222

				295.66		0.8690222

				295.68		0.8690222

				295.7		0.8690222

				295.73		0.8690222

				295.75		0.8690222

				295.77		0.8690222

				295.79		0.8690222

				295.81		0.8690222

				295.83		0.8690222

				295.85		0.8690222

				295.87		0.8690222

				295.89		0.8690222

				295.91		0.8690222

				295.94		0.8690222

				295.96		0.8690222

				295.98		0.8690222

				296		0.8690222

				296.02		0.8690222

				296.04		0.8690222

				296.06		0.8690222

				296.08		0.8690222

				296.1		0.8690222

				296.12		0.8690222

				296.15		0.8690222

				296.17		0.8690222

				296.19		0.8690222

				296.21		0.8690222

				296.23		0.8690222

				296.25		0.8690222

				296.27		0.8690222

				296.29		0.8690222

				296.31		0.8690222

				296.34		0.8690222

				296.36		0.8690222

				296.38		0.8690222

				296.4		0.8742259

				296.42		0.8690222

				296.44		0.8742259

				296.46		0.8742259

				296.48		0.8742259

				296.5		0.8742259

				296.52		0.8742259

				296.55		0.8742259

				296.57		0.8742259

				296.59		0.8742259

				296.61		0.8742259

				296.63		0.8742259

				296.65		0.8742259

				296.67		0.8742259

				296.69		0.8742259

				296.71		0.8742259

				296.74		0.8742259

				296.76		0.8742259

				296.78		0.8742259

				296.8		0.8742259

				296.82		0.8742259

				296.84		0.8742259

				296.86		0.8742259

				296.88		0.8742259

				296.9		0.8742259

				296.92		0.8742259

				296.95		0.8742259

				296.97		0.8742259

				296.99		0.8794297

				297.01		0.8742259

				297.03		0.8742259

				297.05		0.8794297

				297.07		0.8794297

				297.09		0.8742259

				297.11		0.8742259

				297.14		0.8742259

				297.16		0.8794297

				297.18		0.8794297

				297.2		0.8794297

				297.22		0.8794297

				297.24		0.8794297

				297.26		0.8794297

				297.28		0.8794297

				297.3		0.8794297

				297.32		0.8794297

				297.35		0.8794297

				297.37		0.8794297

				297.39		0.8794297

				297.41		0.8794297

				297.43		0.8794297

				297.45		0.8794297

				297.47		0.8794297

				297.49		0.8794297

				297.51		0.8794297

				297.53		0.8794297

				297.56		0.8794297

				297.58		0.8794297

				297.6		0.8794297

				297.62		0.8794297

				297.64		0.8794297

				297.66		0.8794297

				297.68		0.8794297

				297.7		0.8794297

				297.72		0.8742259

				297.75		0.8794297

				297.77		0.8742259

				297.79		0.8742259

				297.81		0.8742259

				297.83		0.8742259

				297.85		0.8742259

				297.87		0.8742259

				297.89		0.8742259

				297.91		0.8742259

				297.93		0.8742259

				297.96		0.8742259

				297.98		0.8742259

				298		0.8742259

				298.02		0.8742259

				298.04		0.8742259

				298.06		0.8742259

				298.08		0.8742259

				298.1		0.8742259

				298.12		0.8742259

				298.15		0.8742259

				298.17		0.8742259

				298.19		0.8742259

				298.21		0.8742259

				298.23		0.8742259

				298.25		0.8742259

				298.27		0.8742259

				298.29		0.8742259

				298.31		0.8742259

				298.33		0.8742259

				298.36		0.8742259

				298.38		0.8742259

				298.4		0.8742259

				298.42		0.8742259

				298.44		0.8742259

				298.46		0.8742259

				298.48		0.8742259

				298.5		0.8742259

				298.52		0.8742259

				298.55		0.8742259

				298.57		0.8742259

				298.59		0.8742259

				298.61		0.8742259

				298.63		0.8742259

				298.65		0.8742259

				298.67		0.8742259

				298.69		0.8742259

				298.71		0.8742259

				298.73		0.8742259

				298.76		0.8742259

				298.78		0.8742259

				298.8		0.8742259

				298.82		0.8742259

				298.84		0.8742259

				298.86		0.8742259

				298.88		0.8742259

				298.9		0.8742259

				298.92		0.8742259

				298.95		0.8742259

				298.97		0.8742259

				298.99		0.8742259

				299.01		0.8742259

				299.03		0.8742259

				299.05		0.8742259

				299.07		0.8742259

				299.09		0.8742259

				299.11		0.8742259

				299.14		0.8742259

				299.16		0.8742259

				299.18		0.8794297

				299.2		0.8794297

				299.22		0.8794297

				299.24		0.8794297

				299.26		0.8742259

				299.28		0.8794297

				299.3		0.8794297

				299.32		0.8742259

				299.35		0.8742259

				299.37		0.8742259

				299.39		0.8742259

				299.41		0.8742259

				299.43		0.8742259

				299.45		0.8742259

				299.47		0.8742259

				299.49		0.8742259

				299.51		0.8742259

				299.54		0.8794297

				299.56		0.8742259

				299.58		0.8742259

				299.6		0.8794297

				299.62		0.8794297

				299.64		0.8794297

				299.66		0.8794297

				299.68		0.8794297

				299.7		0.8794297

				299.73		0.8794297

				299.75		0.8794297

				299.77		0.8794297

				299.79		0.8794297

				299.81		0.8794297

				299.83		0.8794297

				299.85		0.8794297

				299.87		0.8794297

				299.89		0.8794297

				299.91		0.8794297

				299.94		0.8794297

				299.96		0.8794297

				299.98		0.8794297

				300		0.8794297

				300.02		0.8794297

				300.04		0.8794297

				300.06		0.8794297

				300.08		0.8742259

				300.1		0.8742259

				300.13		0.8742259

				300.15		0.8742259

				300.17		0.8742259

				300.19		0.8742259

				300.21		0.8742259

				300.23		0.8742259

				300.25		0.8742259

				300.27		0.8742259

				300.29		0.8742259

				300.31		0.8742259

				300.34		0.8742259

				300.36		0.8742259

				300.38		0.8742259

				300.4		0.8742259

				300.42		0.8742259

				300.44		0.8742259

				300.46		0.8742259

				300.48		0.8742259

				300.5		0.8742259

				300.53		0.8742259

				300.55		0.8742259

				300.57		0.8742259

				300.59		0.8742259

				300.61		0.8742259

				300.63		0.8742259

				300.65		0.8742259

				300.67		0.8742259

				300.69		0.8742259

				300.71		0.8742259

				300.74		0.8742259

				300.76		0.8742259

				300.78		0.8690222

				300.8		0.8690222

				300.82		0.8690222

				300.84		0.8690222

				300.86		0.8690222

				300.88		0.8690222

				300.9		0.8690222

				300.93		0.8690222

				300.95		0.8690222

				300.97		0.8742259

				300.99		0.8690222

				301.01		0.8690222

				301.03		0.8690222

				301.05		0.8690222

				301.07		0.8690222

				301.09		0.8690222

				301.11		0.8690222

				301.14		0.8690222

				301.16		0.8690222

				301.18		0.8690222

				301.2		0.8690222

				301.22		0.8690222

				301.24		0.8638185

				301.26		0.8638185

				301.28		0.8638185

				301.3		0.8638185

				301.32		0.8638185

				301.35		0.8638185

				301.37		0.8638185

				301.39		0.8638185

				301.41		0.8638185

				301.43		0.8638185

				301.45		0.8638185

				301.47		0.8638185

				301.49		0.8638185

				301.51		0.8638185

				301.54		0.8638185

				301.56		0.8638185

				301.58		0.8638185

				301.6		0.8638185

				301.62		0.8638185

				301.64		0.8586148

				301.66		0.8586148

				301.68		0.8586148

				301.7		0.8586148

				301.72		0.8586148

				301.75		0.8586148

				301.77		0.8586148

				301.79		0.8586148

				301.81		0.8586148

				301.83		0.8586148

				301.85		0.8586148

				301.87		0.8586148

				301.89		0.8586148

				301.91		0.8586148

				301.94		0.8586148

				301.96		0.8586148

				301.98		0.8586148

				302		0.8586148

				302.02		0.8586148

				302.04		0.8586148

				302.06		0.8586148

				302.08		0.8586148

				302.1		0.8586148

				302.12		0.8586148

				302.15		0.853411

				302.17		0.853411

				302.19		0.853411

				302.21		0.853411

				302.23		0.853411

				302.25		0.853411

				302.27		0.853411

				302.29		0.853411

				302.31		0.853411

				302.34		0.853411

				302.36		0.853411

				302.38		0.853411

				302.4		0.853411

				302.42		0.853411

				302.44		0.853411

				302.46		0.853411

				302.48		0.853411

				302.5		0.853411

				302.52		0.853411

				302.55		0.853411

				302.57		0.853411

				302.59		0.853411

				302.61		0.853411

				302.63		0.853411

				302.65		0.853411

				302.67		0.8482073

				302.69		0.853411

				302.71		0.853411

				302.74		0.853411

				302.76		0.853411

				302.78		0.853411

				302.8		0.853411

				302.82		0.8482073

				302.84		0.853411

				302.86		0.8482073

				302.88		0.8482073

				302.9		0.8482073

				302.92		0.8482073

				302.95		0.8482073

				302.97		0.8482073

				302.99		0.8482073

				303.01		0.8482073

				303.03		0.8482073

				303.05		0.8482073

				303.07		0.8482073

				303.09		0.8482073

				303.11		0.8482073

				303.14		0.8482073

				303.16		0.8482073

				303.18		0.8482073

				303.2		0.8482073

				303.22		0.8482073

				303.24		0.8482073

				303.26		0.8482073

				303.28		0.8482073

				303.3		0.8482073

				303.33		0.8482073

				303.35		0.8482073

				303.37		0.8482073

				303.39		0.8482073

				303.41		0.8482073

				303.43		0.8482073

				303.45		0.8482073

				303.47		0.8482073

				303.49		0.8482073

				303.52		0.8482073

				303.54		0.8430036

				303.56		0.8430036

				303.58		0.8430036

				303.6		0.8430036

				303.62		0.8430036

				303.64		0.8430036

				303.66		0.8430036

				303.68		0.8482073

				303.71		0.8430036

				303.73		0.8430036

				303.75		0.8430036

				303.77		0.8430036

				303.79		0.8430036

				303.81		0.8430036

				303.83		0.8430036

				303.85		0.8430036

				303.87		0.8430036

				303.9		0.8430036

				303.92		0.8430036

				303.94		0.8430036

				303.96		0.8430036

				303.98		0.8430036

				304		0.8430036

				304.02		0.8430036

				304.04		0.8430036

				304.06		0.8430036

				304.08		0.8430036

				304.11		0.8430036

				304.13		0.8430036

				304.15		0.8430036

				304.17		0.8430036

				304.19		0.8430036

				304.21		0.8430036

				304.23		0.8430036

				304.25		0.8430036

				304.27		0.8430036

				304.3		0.8430036

				304.32		0.8430036

				304.34		0.8430036

				304.36		0.8430036

				304.38		0.8430036

				304.4		0.8430036

				304.42		0.8430036

				304.44		0.8430036

				304.46		0.8430036

				304.49		0.8430036

				304.51		0.8430036

				304.53		0.8430036

				304.55		0.8430036

				304.57		0.8377999

				304.59		0.8430036

				304.61		0.8430036

				304.63		0.8377999

				304.65		0.8377999

				304.68		0.8377999

				304.7		0.8377999

				304.72		0.8430036

				304.74		0.8430036

				304.76		0.8430036

				304.78		0.8430036

				304.8		0.8377999

				304.82		0.8377999

				304.84		0.8377999

				304.87		0.8430036

				304.89		0.8377999

				304.91		0.8430036

				304.93		0.8377999

				304.95		0.8430036

				304.97		0.8377999

				304.99		0.8377999

				305.01		0.8430036

				305.03		0.8430036

				305.06		0.8430036

				305.08		0.8377999

				305.1		0.8377999

				305.12		0.8377999

				305.14		0.8377999

				305.16		0.8377999

				305.18		0.8377999

				305.2		0.8377999

				305.22		0.8377999

				305.25		0.8377999

				305.27		0.8377999

				305.29		0.8377999

				305.31		0.8377999

				305.33		0.8377999

				305.35		0.8377999

				305.37		0.8377999

				305.39		0.8377999

				305.41		0.8377999

				305.44		0.8377999

				305.46		0.8377999

				305.48		0.8377999

				305.5		0.8377999

				305.52		0.8377999

				305.54		0.8377999

				305.56		0.8325961

				305.58		0.8377999

				305.6		0.8325961

				305.62		0.8377999

				305.65		0.8377999

				305.67		0.8377999

				305.69		0.8325961

				305.71		0.8377999

				305.73		0.8377999

				305.75		0.8377999

				305.77		0.8325961

				305.79		0.8377999

				305.81		0.8377999

				305.84		0.8325961

				305.86		0.8377999

				305.88		0.8377999

				305.9		0.8377999

				305.92		0.8377999

				305.94		0.8377999

				305.96		0.8377999

				305.98		0.8325961

				306		0.8377999

				306.03		0.8377999

				306.05		0.8377999

				306.07		0.8377999

				306.09		0.8377999

				306.11		0.8377999

				306.13		0.8377999

				306.15		0.8377999

				306.17		0.8377999

				306.19		0.8377999

				306.22		0.8377999

				306.24		0.8377999

				306.26		0.8377999

				306.28		0.8377999

				306.3		0.8377999

				306.32		0.8377999

				306.34		0.8377999

				306.36		0.8325961

				306.38		0.8377999

				306.41		0.8377999

				306.43		0.8377999

				306.45		0.8377999

				306.47		0.8377999

				306.49		0.8377999

				306.51		0.8377999

				306.53		0.8377999

				306.55		0.8377999

				306.57		0.8377999

				306.6		0.8377999

				306.62		0.8377999

				306.64		0.8377999

				306.66		0.8377999

				306.68		0.8377999

				306.7		0.8377999

				306.72		0.8377999

				306.74		0.8377999

				306.76		0.8377999

				306.79		0.8377999

				306.81		0.8377999

				306.83		0.8377999

				306.85		0.8377999

				306.87		0.8377999

				306.89		0.8377999

				306.91		0.8377999

				306.93		0.8377999

				306.95		0.8377999

				306.98		0.8377999

				307		0.8377999

				307.02		0.8377999

				307.04		0.8377999

				307.06		0.8377999

				307.08		0.8377999

				307.1		0.8377999

				307.12		0.8377999

				307.14		0.8377999

				307.17		0.8377999

				307.19		0.8377999

				307.21		0.8377999

				307.23		0.8377999

				307.25		0.8377999

				307.27		0.8377999

				307.29		0.8377999

				307.31		0.8377999

				307.33		0.8377999

				307.36		0.8377999

				307.38		0.8377999

				307.4		0.8377999

				307.42		0.8377999

				307.44		0.8377999

				307.46		0.8377999

				307.48		0.8377999

				307.5		0.8377999

				307.52		0.8377999

				307.55		0.8377999

				307.57		0.8377999

				307.59		0.8377999

				307.61		0.8430036

				307.63		0.8377999

				307.65		0.8377999

				307.67		0.8430036

				307.69		0.8430036

				307.71		0.8430036

				307.74		0.8430036

				307.76		0.8430036

				307.78		0.8430036

				307.8		0.8377999

				307.82		0.8377999

				307.84		0.8377999

				307.86		0.8377999

				307.88		0.8377999

				307.9		0.8377999

				307.93		0.8377999

				307.95		0.8377999

				307.97		0.8377999

				307.99		0.8377999

				308.01		0.8377999

				308.03		0.8377999

				308.05		0.8377999

				308.07		0.8377999

				308.09		0.8377999

				308.12		0.8377999

				308.14		0.8377999

				308.16		0.8377999

				308.18		0.8377999

				308.2		0.8377999

				308.22		0.8377999

				308.24		0.8377999

				308.26		0.8377999

				308.28		0.8377999

				308.31		0.8377999

				308.33		0.8377999

				308.35		0.8377999

				308.37		0.8377999

				308.39		0.8377999

				308.41		0.8377999

				308.43		0.8377999

				308.45		0.8377999

				308.47		0.8377999

				308.5		0.8325961

				308.52		0.8325961

				308.54		0.8325961

				308.56		0.8325961

				308.58		0.8325961

				308.6		0.8325961

				308.62		0.8325961

				308.64		0.8325961

				308.66		0.8325961

				308.69		0.8325961

				308.71		0.8325961

				308.73		0.8325961

				308.75		0.8325961

				308.77		0.8325961

				308.79		0.8325961

				308.81		0.8325961

				308.83		0.8273924

				308.85		0.8325961

				308.88		0.8273924

				308.9		0.8273924

				308.92		0.8325961

				308.94		0.8273924

				308.96		0.8325961

				308.98		0.8273924

				309		0.8325961

				309.02		0.8273924

				309.04		0.8273924

				309.07		0.8273924

				309.09		0.8273924

				309.11		0.8273924

				309.13		0.8273924

				309.15		0.8273924

				309.17		0.8273924

				309.19		0.8273924

				309.21		0.8273924

				309.23		0.8273924

				309.26		0.8273924

				309.28		0.8273924

				309.3		0.8273924

				309.32		0.8221887

				309.34		0.8273924

				309.36		0.8221887

				309.38		0.8221887

				309.4		0.8221887

				309.42		0.8221887

				309.45		0.8221887

				309.47		0.8221887

				309.49		0.8221887

				309.51		0.8221887

				309.53		0.8221887

				309.55		0.8221887

				309.57		0.8221887

				309.59		0.8221887

				309.61		0.8221887

				309.64		0.8221887

				309.66		0.8221887

				309.68		0.8221887

				309.7		0.8221887

				309.72		0.8221887

				309.74		0.8221887

				309.76		0.8221887

				309.78		0.8221887

				309.8		0.8221887

				309.83		0.8221887

				309.85		0.8221887

				309.87		0.8221887

				309.89		0.8221887

				309.91		0.8221887

				309.93		0.8221887

				309.95		0.8221887

				309.97		0.8221887

				309.99		0.8221887

				310.02		0.8221887

				310.04		0.816985

				310.06		0.816985

				310.08		0.816985

				310.1		0.816985

				310.12		0.816985

				310.14		0.816985

				310.16		0.816985

				310.19		0.816985

				310.21		0.816985

				310.23		0.816985

				310.25		0.816985

				310.27		0.816985

				310.29		0.816985

				310.31		0.816985

				310.33		0.816985

				310.35		0.816985

				310.38		0.816985

				310.4		0.816985

				310.42		0.816985

				310.44		0.816985

				310.46		0.816985

				310.48		0.816985

				310.5		0.816985

				310.52		0.816985

				310.54		0.816985

				310.57		0.816985

				310.59		0.816985

				310.61		0.816985

				310.63		0.816985

				310.65		0.8221887

				310.67		0.816985

				310.69		0.8221887

				310.71		0.8221887

				310.73		0.816985

				310.76		0.8221887

				310.78		0.816985

				310.8		0.816985

				310.82		0.816985

				310.84		0.816985

				310.86		0.816985

				310.88		0.816985

				310.9		0.816985

				310.92		0.816985

				310.95		0.816985

				310.97		0.816985

				310.99		0.816985

				311.01		0.816985

				311.03		0.816985

				311.05		0.816985

				311.07		0.816985

				311.09		0.816985

				311.12		0.816985

				311.14		0.816985

				311.16		0.816985

				311.18		0.816985

				311.2		0.816985

				311.22		0.816985

				311.24		0.816985

				311.26		0.816985

				311.28		0.816985

				311.31		0.816985

				311.33		0.816985

				311.35		0.816985

				311.37		0.816985

				311.39		0.816985

				311.41		0.816985

				311.43		0.816985

				311.45		0.816985

				311.47		0.816985

				311.5		0.816985

				311.52		0.816985

				311.54		0.816985

				311.56		0.816985

				311.58		0.816985

				311.6		0.816985

				311.62		0.816985

				311.64		0.816985

				311.66		0.816985

				311.69		0.8221887

				311.71		0.8221887

				311.73		0.8221887

				311.75		0.8221887

				311.77		0.8221887

				311.79		0.816985

				311.81		0.8221887

				311.83		0.8221887

				311.85		0.8221887

				311.88		0.816985

				311.9		0.816985

				311.92		0.816985

				311.94		0.816985

				311.96		0.816985

				311.98		0.816985

				312		0.8221887

				312.02		0.816985

				312.05		0.8221887

				312.07		0.8221887

				312.09		0.8221887

				312.11		0.8221887

				312.13		0.8221887

				312.15		0.8221887

				312.17		0.8221887

				312.19		0.8221887

				312.21		0.8221887

				312.24		0.8221887

				312.26		0.8221887

				312.28		0.8221887

				312.3		0.8221887

				312.32		0.8221887

				312.34		0.8221887

				312.36		0.8221887

				312.38		0.8221887

				312.4		0.8221887

				312.43		0.8221887

				312.45		0.8221887

				312.47		0.8221887

				312.49		0.8221887

				312.51		0.8221887

				312.53		0.8221887

				312.55		0.8221887

				312.57		0.8221887

				312.6		0.8221887

				312.62		0.8221887

				312.64		0.8221887

				312.66		0.8221887

				312.68		0.8221887

				312.7		0.8221887

				312.72		0.8221887

				312.74		0.8221887

				312.76		0.8221887

				312.79		0.8221887

				312.81		0.8221887

				312.83		0.8221887

				312.85		0.8221887

				312.87		0.8221887

				312.89		0.8221887

				312.91		0.8221887

				312.93		0.8221887

				312.95		0.8221887

				312.98		0.8221887

				313		0.8221887

				313.02		0.8221887

				313.04		0.8221887

				313.06		0.8221887

				313.08		0.8221887

				313.1		0.8221887

				313.12		0.8221887

				313.14		0.8221887

				313.17		0.8221887

				313.19		0.8221887

				313.21		0.8221887

				313.23		0.8221887

				313.25		0.8221887

				313.27		0.8221887

				313.29		0.8221887

				313.31		0.8221887

				313.34		0.8221887

				313.36		0.8221887

				313.38		0.8221887

				313.4		0.8221887

				313.42		0.8221887

				313.44		0.8221887

				313.46		0.8221887

				313.48		0.8221887

				313.5		0.8221887

				313.53		0.8221887

				313.55		0.8221887

				313.57		0.8221887

				313.59		0.8221887

				313.61		0.8221887

				313.63		0.8221887

				313.65		0.8221887

				313.67		0.8221887

				313.69		0.8221887

				313.72		0.8221887

				313.74		0.8221887

				313.76		0.8221887

				313.78		0.8221887

				313.8		0.8221887

				313.82		0.8221887

				313.84		0.8221887

				313.86		0.8221887

				313.88		0.8221887

				313.91		0.8221887

				313.93		0.8221887

				313.95		0.8221887

				313.97		0.8221887

				313.99		0.8221887

				314.01		0.8221887

				314.03		0.8221887

				314.05		0.8221887

				314.08		0.8221887

				314.1		0.8221887

				314.12		0.8221887

				314.14		0.8221887

				314.16		0.8221887

				314.18		0.8221887

				314.2		0.8221887

				314.22		0.8221887

				314.24		0.8221887

				314.27		0.8221887

				314.29		0.8221887

				314.31		0.8221887

				314.33		0.8221887

				314.35		0.8221887

				314.37		0.8221887

				314.39		0.8221887

				314.41		0.8221887

				314.43		0.8221887

				314.46		0.8221887

				314.48		0.8221887

				314.5		0.8221887

				314.52		0.8221887

				314.54		0.8221887

				314.56		0.8221887

				314.58		0.8221887

				314.6		0.8221887

				314.62		0.8221887

				314.65		0.8221887

				314.67		0.816985

				314.69		0.816985

				314.71		0.8221887

				314.73		0.8221887

				314.75		0.8221887

				314.77		0.8221887

				314.79		0.8221887

				314.82		0.8221887

				314.84		0.8221887

				314.86		0.8221887

				314.88		0.8221887

				314.9		0.8221887

				314.92		0.8221887

				314.94		0.8221887

				314.96		0.8221887

				314.98		0.816985

				315.01		0.816985

				315.03		0.8221887

				315.05		0.8221887

				315.07		0.816985

				315.09		0.8221887

				315.11		0.8221887

				315.13		0.816985

				315.15		0.816985

				315.17		0.8221887

				315.2		0.8221887

				315.22		0.816985

				315.24		0.8221887

				315.26		0.816985

				315.28		0.8221887

				315.3		0.8221887

				315.32		0.8221887

				315.34		0.816985

				315.37		0.816985

				315.39		0.8221887

				315.41		0.816985

				315.43		0.816985

				315.45		0.816985

				315.47		0.816985

				315.49		0.816985

				315.51		0.816985

				315.53		0.816985

				315.56		0.816985

				315.58		0.816985

				315.6		0.816985

				315.62		0.816985

				315.64		0.816985

				315.66		0.816985

				315.68		0.816985

				315.7		0.816985

				315.73		0.816985

				315.75		0.8117812

				315.77		0.8117812

				315.79		0.816985

				315.81		0.8117812

				315.83		0.8117812

				315.85		0.8117812

				315.87		0.8117812

				315.89		0.8117812

				315.92		0.8117812

				315.94		0.8117812

				315.96		0.8117812

				315.98		0.8117812

				316		0.8117812

				316.02		0.8117812

				316.04		0.8117812

				316.06		0.8117812

				316.08		0.8117812

				316.11		0.8117812

				316.13		0.8117812

				316.15		0.8117812

				316.17		0.8065775

				316.19		0.8065775

				316.21		0.8065775

				316.23		0.8065775

				316.25		0.8065775

				316.28		0.8065775

				316.3		0.8065775

				316.32		0.8065775

				316.34		0.8065775

				316.36		0.8065775

				316.38		0.8065775

				316.4		0.8065775

				316.42		0.8065775

				316.44		0.8065775

				316.47		0.8065775

				316.49		0.8065775

				316.51		0.8065775

				316.53		0.8065775

				316.55		0.8065775

				316.57		0.8065775

				316.59		0.8065775

				316.61		0.8013738

				316.63		0.8013738

				316.66		0.8013738

				316.68		0.8065775

				316.7		0.8065775

				316.72		0.8065775

				316.74		0.8065775

				316.76		0.8065775

				316.78		0.8065775

				316.8		0.8065775

				316.82		0.8065775

				316.85		0.8065775

				316.87		0.8065775

				316.89		0.8065775

				316.91		0.8065775

				316.93		0.8013738

				316.95		0.8013738

				316.97		0.8013738

				316.99		0.8013738

				317.01		0.8013738

				317.04		0.8013738

				317.06		0.8013738

				317.08		0.8013738

				317.1		0.8013738

				317.12		0.8013738

				317.14		0.8013738

				317.16		0.8013738

				317.18		0.8013738

				317.21		0.8013738

				317.23		0.8013738

				317.25		0.8013738

				317.27		0.8013738

				317.29		0.8013738

				317.31		0.8013738

				317.33		0.8013738

				317.35		0.8013738

				317.37		0.8013738

				317.4		0.8013738

				317.42		0.8013738

				317.44		0.7961701

				317.46		0.7961701

				317.48		0.7961701

				317.5		0.7961701

				317.52		0.7961701

				317.54		0.7961701

				317.56		0.7961701

				317.59		0.7961701

				317.61		0.7961701

				317.63		0.7961701

				317.65		0.7961701

				317.67		0.7961701

				317.69		0.7961701

				317.71		0.7961701

				317.73		0.7961701

				317.75		0.7961701

				317.78		0.7961701

				317.8		0.7961701

				317.82		0.7961701

				317.84		0.7961701

				317.86		0.7909663

				317.88		0.7909663

				317.9		0.7909663

				317.92		0.7961701

				317.95		0.7961701

				317.97		0.7961701

				317.99		0.7961701

				318.01		0.7961701

				318.03		0.7961701

				318.05		0.7961701

				318.07		0.7961701

				318.09		0.7961701

				318.11		0.7961701

				318.14		0.7961701

				318.16		0.7909663

				318.18		0.7909663

				318.2		0.7909663

				318.22		0.7909663

				318.24		0.7961701

				318.26		0.7961701

				318.28		0.7961701

				318.3		0.7961701

				318.33		0.7961701

				318.35		0.7961701

				318.37		0.7961701

				318.39		0.7961701

				318.41		0.7961701

				318.43		0.7909663

				318.45		0.7961701

				318.47		0.7961701

				318.5		0.7909663

				318.52		0.7961701

				318.54		0.7961701

				318.56		0.7961701

				318.58		0.7961701

				318.6		0.7961701

				318.62		0.7961701

				318.64		0.7961701

				318.66		0.7909663

				318.69		0.7909663

				318.71		0.7909663

				318.73		0.7909663

				318.75		0.7909663

				318.77		0.7909663

				318.79		0.7909663

				318.81		0.7909663

				318.83		0.7909663

				318.85		0.7909663

				318.88		0.7909663

				318.9		0.7961701

				318.92		0.7909663

				318.94		0.7857626

				318.96		0.7753552

				318.98		0.7753552

				319		0.7753552

				319.02		0.7753552

				319.05		0.7753552

				319.07		0.7753552

				319.09		0.7753552

				319.11		0.7753552

				319.13		0.7701514

				319.15		0.7701514

				319.17		0.7701514

				319.19		0.7701514

				319.21		0.7701514

				319.24		0.7649477

				319.26		0.7649477

				319.28		0.7649477

				319.3		0.7649477

				319.32		0.7649477

				319.34		0.7701514

				319.36		0.7701514

				319.38		0.7701514

				319.41		0.7701514

				319.43		0.7701514

				319.45		0.7701514

				319.47		0.7701514

				319.49		0.7701514

				319.51		0.7753552

				319.53		0.7753552

				319.55		0.7753552

				319.57		0.7753552

				319.6		0.7753552

				319.62		0.7753552

				319.64		0.7805589

				319.66		0.7805589

				319.68		0.7857626

				319.7		0.7909663

				319.72		0.7909663

				319.74		0.7961701

				319.76		0.7961701

				319.79		0.7961701

				319.81		0.7961701

				319.83		0.7961701

				319.85		0.8013738

				319.87		0.7961701

				319.89		0.7961701

				319.91		0.7961701

				319.93		0.7961701

				319.95		0.7961701

				319.98		0.8013738

				320		0.7961701

				320.02		0.7961701

				320.04		0.7961701

				320.06		0.7961701

				320.08		0.7961701

				320.1		0.7961701

				320.12		0.7961701

				320.14		0.7961701

				320.17		0.7961701

				320.19		0.7961701

				320.21		0.7961701

				320.23		0.7961701

				320.25		0.8013738

				320.27		0.8013738

				320.29		0.8013738

				320.31		0.7961701

				320.33		0.8013738

				320.36		0.8013738

				320.38		0.8013738

				320.4		0.8013738

				320.42		0.8013738

				320.44		0.8013738

				320.46		0.8013738

				320.48		0.7961701

				320.5		0.816985

				320.53		0.8117812

				320.55		0.8273924

				320.57		0.8325961

				320.59		0.8377999

				320.61		0.8325961

				320.63		0.8325961

				320.65		0.8273924

				320.67		0.8273924

				320.69		0.8273924

				320.72		0.8221887

				320.74		0.8221887

				320.76		0.8221887

				320.78		0.816985

				320.8		0.816985

				320.82		0.816985

				320.84		0.816985

				320.86		0.8117812

				320.88		0.8117812

				320.91		0.8117812

				320.93		0.8117812

				320.95		0.8117812

				320.97		0.8117812

				320.99		0.8117812

				321.01		0.8065775

				321.03		0.8065775

				321.05		0.8117812

				321.08		0.8117812

				321.1		0.8117812

				321.12		0.8117812

				321.14		0.8117812

				321.16		0.8117812

				321.18		0.8117812

				321.2		0.8117812

				321.22		0.8117812

				321.25		0.8117812

				321.27		0.8117812

				321.29		0.8117812

				321.31		0.8117812

				321.33		0.8117812

				321.35		0.8065775

				321.37		0.7909663

				321.39		0.7805589

				321.41		0.7805589

				321.44		0.7805589

				321.46		0.7805589

				321.48		0.7805589

				321.5		0.7753552

				321.52		0.7753552

				321.54		0.7753552

				321.56		0.7753552

				321.58		0.7753552

				321.61		0.7753552

				321.63		0.7753552

				321.65		0.7753552

				321.67		0.7753552

				321.69		0.7753552

				321.71		0.7753552

				321.73		0.7753552

				321.75		0.7753552

				321.77		0.7753552

				321.8		0.7753552

				321.82		0.7753552

				321.84		0.7753552

				321.86		0.7753552

				321.88		0.7753552

				321.9		0.7753552

				321.92		0.7753552

				321.94		0.7753552

				321.97		0.7753552

				321.99		0.7753552

				322.01		0.7753552

				322.03		0.7753552

				322.05		0.7753552

				322.07		0.7753552

				322.09		0.7753552

				322.11		0.7753552

				322.13		0.7753552

				322.16		0.7753552

				322.18		0.7753552

				322.2		0.7753552

				322.22		0.7753552

				322.24		0.7753552

				322.26		0.7753552

				322.28		0.7701514

				322.3		0.7701514

				322.33		0.7701514

				322.35		0.7701514

				322.37		0.7701514

				322.39		0.7753552

				322.41		0.7701514

				322.43		0.7701514

				322.45		0.7701514

				322.47		0.7701514

				322.49		0.7701514

				322.52		0.7753552

				322.54		0.7753552

				322.56		0.7753552

				322.58		0.7753552

				322.6		0.7753552

				322.62		0.7753552

				322.64		0.7753552

				322.66		0.7753552

				322.69		0.7753552

				322.71		0.7701514

				322.73		0.7701514

				322.75		0.7701514

				322.77		0.7701514

				322.79		0.7701514

				322.81		0.7701514

				322.83		0.7701514

				322.85		0.7701514

				322.88		0.7701514

				322.9		0.7701514

				322.92		0.7701514

				322.94		0.7701514

				322.96		0.7701514

				322.98		0.7701514

				323		0.7701514

				323.02		0.7701514

				323.04		0.7701514

				323.07		0.7701514

				323.09		0.7701514

				323.11		0.7701514

				323.13		0.7701514

				323.15		0.7701514

				323.17		0.7649477

				323.19		0.7701514

				323.21		0.7701514

				323.24		0.7701514

				323.26		0.7649477

				323.28		0.7649477

				323.3		0.7701514

				323.32		0.7701514

				323.34		0.7649477

				323.36		0.7701514

				323.38		0.7649477

				323.4		0.7649477

				323.43		0.7649477

				323.45		0.7649477

				323.47		0.7649477

				323.49		0.7649477

				323.51		0.7649477

				323.53		0.7649477

				323.55		0.7649477

				323.57		0.7649477

				323.6		0.7649477

				323.62		0.7649477

				323.64		0.7649477

				323.66		0.7649477

				323.68		0.7649477

				323.7		0.7649477

				323.72		0.7649477

				323.74		0.7649477

				323.76		0.7649477

				323.79		0.7649477

				323.81		0.7649477

				323.83		0.7649477

				323.85		0.7649477

				323.87		0.7649477

				323.89		0.7649477

				323.91		0.7649477

				323.93		0.7649477

				323.96		0.7649477

				323.98		0.7649477

				324		0.7649477

				324.02		0.7649477

				324.04		0.7649477

				324.06		0.7649477

				324.08		0.7649477

				324.1		0.7649477

				324.12		0.7649477

				324.15		0.7649477

				324.17		0.7649477

				324.19		0.7649477

				324.21		0.7649477

				324.23		0.7649477

				324.25		0.7649477

				324.27		0.7649477

				324.29		0.7649477

				324.31		0.7649477

				324.34		0.7649477

				324.36		0.7649477

				324.38		0.7649477

				324.4		0.7649477

				324.42		0.7649477

				324.44		0.7649477

				324.46		0.7649477

				324.48		0.7649477

				324.51		0.7649477

				324.53		0.7649477

				324.55		0.7649477

				324.57		0.7649477

				324.59		0.7649477

				324.61		0.7649477

				324.63		0.759744

				324.65		0.7649477

				324.67		0.7649477

				324.7		0.7649477

				324.72		0.759744

				324.74		0.759744

				324.76		0.759744

				324.78		0.7649477

				324.8		0.759744

				324.82		0.7649477

				324.84		0.7649477

				324.87		0.759744

				324.89		0.759744

				324.91		0.759744

				324.93		0.7649477

				324.95		0.7649477

				324.97		0.7649477

				324.99		0.7649477

				325.01		0.7649477

				325.03		0.7649477

				325.06		0.7649477

				325.08		0.7649477

				325.1		0.7649477

				325.12		0.7649477

				325.14		0.7649477

				325.16		0.7649477

				325.18		0.7649477

				325.2		0.7649477

				325.23		0.7649477

				325.25		0.7649477

				325.27		0.7649477

				325.29		0.759744

				325.31		0.759744

				325.33		0.759744

				325.35		0.7649477

				325.37		0.759744

				325.39		0.759744

				325.42		0.759744

				325.44		0.759744

				325.46		0.759744

				325.48		0.7649477

				325.5		0.759744

				325.52		0.759744

				325.54		0.7649477

				325.56		0.759744

				325.59		0.759744

				325.61		0.759744

				325.63		0.759744

				325.65		0.759744

				325.67		0.759744

				325.69		0.759744

				325.71		0.759744

				325.73		0.759744

				325.75		0.759744

				325.78		0.759744

				325.8		0.759744

				325.82		0.759744

				325.84		0.759744

				325.86		0.759744

				325.88		0.759744

				325.9		0.759744

				325.92		0.759744

				325.95		0.759744

				325.97		0.759744

				325.99		0.759744

				326.01		0.759744

				326.03		0.759744

				326.05		0.759744

				326.07		0.759744

				326.09		0.759744

				326.12		0.759744

				326.14		0.759744

				326.16		0.759744

				326.18		0.759744

				326.2		0.759744

				326.22		0.759744

				326.24		0.759744

				326.26		0.759744

				326.28		0.759744

				326.31		0.759744

				326.33		0.759744

				326.35		0.759744

				326.37		0.759744

				326.39		0.759744

				326.41		0.759744

				326.43		0.759744

				326.45		0.759744

				326.48		0.759744

				326.5		0.759744

				326.52		0.759744

				326.54		0.759744

				326.56		0.759744

				326.58		0.759744

				326.6		0.759744

				326.62		0.759744

				326.64		0.759744

				326.67		0.759744

				326.69		0.759744

				326.71		0.759744

				326.73		0.759744

				326.75		0.759744

				326.77		0.759744

				326.79		0.759744

				326.81		0.759744

				326.84		0.759744

				326.86		0.759744

				326.88		0.759744

				326.9		0.759744

				326.92		0.759744

				326.94		0.759744

				326.96		0.759744

				326.98		0.759744

				327		0.759744

				327.03		0.759744

				327.05		0.759744

				327.07		0.7545403

				327.09		0.7545403

				327.11		0.7545403

				327.13		0.7545403

				327.15		0.7545403

				327.17		0.7545403

				327.2		0.7545403

				327.22		0.7545403

				327.24		0.7545403

				327.26		0.7545403

				327.28		0.7545403

				327.3		0.7545403

				327.32		0.7545403

				327.34		0.7545403

				327.36		0.7545403

				327.39		0.7545403

				327.41		0.7545403

				327.43		0.7545403

				327.45		0.7545403

				327.47		0.7545403

				327.49		0.7545403

				327.51		0.7545403

				327.53		0.7545403

				327.56		0.7545403

				327.58		0.7545403

				327.6		0.7545403

				327.62		0.7545403

				327.64		0.7545403

				327.66		0.7545403

				327.68		0.7545403

				327.7		0.7545403

				327.73		0.7545403

				327.75		0.7545403

				327.77		0.7545403

				327.79		0.7545403

				327.81		0.7545403

				327.83		0.7545403

				327.85		0.7545403

				327.87		0.7545403

				327.89		0.7545403

				327.92		0.7545403

				327.94		0.7545403

				327.96		0.7545403

				327.98		0.7545403

				328		0.7545403

				328.02		0.7545403

				328.04		0.7545403

				328.06		0.7545403

				328.09		0.7493365

				328.11		0.7493365

				328.13		0.7493365

				328.15		0.7493365

				328.17		0.7493365

				328.19		0.7493365

				328.21		0.7493365

				328.23		0.7493365

				328.25		0.7493365

				328.28		0.7493365

				328.3		0.7493365

				328.32		0.7493365

				328.34		0.7493365

				328.36		0.7493365

				328.38		0.7493365

				328.4		0.7493365

				328.42		0.7493365

				328.45		0.7493365

				328.47		0.7493365

				328.49		0.7493365

				328.51		0.7493365

				328.53		0.7493365

				328.55		0.7493365

				328.57		0.7493365

				328.59		0.7441328

				328.61		0.7493365

				328.64		0.7493365

				328.66		0.7493365

				328.68		0.7493365

				328.7		0.7493365

				328.72		0.7493365

				328.74		0.7493365

				328.76		0.7493365

				328.78		0.7493365

				328.8		0.7441328

				328.83		0.7441328

				328.85		0.7493365

				328.87		0.7441328

				328.89		0.7441328

				328.91		0.7441328

				328.93		0.7441328

				328.95		0.7441328

				328.97		0.7441328

				328.99		0.7441328

				329.02		0.7441328

				329.04		0.7493365

				329.06		0.7493365

				329.08		0.7493365

				329.1		0.7493365

				329.12		0.7493365

				329.14		0.7493365

				329.16		0.7493365

				329.19		0.7493365

				329.21		0.7493365

				329.23		0.7493365

				329.25		0.7493365

				329.27		0.7493365

				329.29		0.7493365

				329.31		0.7493365

				329.33		0.7493365

				329.35		0.7493365

				329.38		0.7493365

				329.4		0.7493365

				329.42		0.7493365

				329.44		0.7493365

				329.46		0.7493365

				329.48		0.7493365

				329.5		0.7493365

				329.52		0.7493365

				329.54		0.7493365

				329.57		0.7493365

				329.59		0.7493365

				329.61		0.7441328

				329.63		0.7441328

				329.65		0.7441328

				329.67		0.7441328

				329.69		0.7441328

				329.71		0.7441328

				329.74		0.7441328

				329.76		0.7441328

				329.78		0.7441328

				329.8		0.7441328

				329.82		0.7441328

				329.84		0.7493365

				329.86		0.7493365

				329.88		0.7441328

				329.9		0.7441328

				329.93		0.7493365

				329.95		0.7493365

				329.97		0.7493365

				329.99		0.7493365

				330.01		0.7493365

				330.03		0.7493365

				330.05		0.7493365

				330.07		0.7493365

				330.09		0.7493365

				330.12		0.7493365

				330.14		0.7493365

				330.16		0.7493365

				330.18		0.7493365

				330.2		0.7441328

				330.22		0.7493365

				330.24		0.7493365

				330.26		0.7493365

				330.29		0.7493365

				330.31		0.7493365

				330.33		0.7493365

				330.35		0.7441328

				330.37		0.7441328

				330.39		0.7493365

				330.41		0.7493365

				330.43		0.7493365

				330.45		0.7493365

				330.48		0.7493365

				330.5		0.7441328

				330.52		0.7441328

				330.54		0.7441328

				330.56		0.7441328

				330.58		0.7441328

				330.6		0.7441328

				330.62		0.7441328

				330.64		0.7441328

				330.67		0.7441328

				330.69		0.7441328

				330.71		0.7441328

				330.73		0.7441328

				330.75		0.7441328

				330.77		0.7441328

				330.79		0.7441328

				330.81		0.7441328

				330.84		0.7493365

				330.86		0.7493365

				330.88		0.7493365

				330.9		0.7493365

				330.92		0.7493365

				330.94		0.7493365

				330.96		0.7493365

				330.98		0.7493365

				331		0.7493365

				331.03		0.7493365

				331.05		0.7493365

				331.07		0.7493365

				331.09		0.7493365

				331.11		0.7493365

				331.13		0.7441328

				331.15		0.7441328

				331.17		0.7441328

				331.19		0.7441328

				331.22		0.7441328

				331.24		0.7441328

				331.26		0.7441328

				331.28		0.7441328

				331.3		0.7441328

				331.32		0.7441328

				331.34		0.7441328

				331.36		0.7441328

				331.38		0.7441328

				331.41		0.7441328

				331.43		0.7441328

				331.45		0.7441328

				331.47		0.7441328

				331.49		0.7441328

				331.51		0.7441328

				331.53		0.7441328

				331.55		0.7441328

				331.58		0.7441328

				331.6		0.7441328

				331.62		0.7389291

				331.64		0.7389291

				331.66		0.7389291

				331.68		0.7389291

				331.7		0.7389291

				331.72		0.7389291

				331.74		0.7441328

				331.77		0.7441328

				331.79		0.7441328

				331.81		0.7389291

				331.83		0.7441328

				331.85		0.7441328

				331.87		0.7441328

				331.89		0.7441328

				331.91		0.7441328

				331.93		0.7389291

				331.96		0.7389291

				331.98		0.7389291

				332		0.7389291

				332.02		0.7389291

				332.04		0.7389291

				332.06		0.7389291

				332.08		0.7389291

				332.1		0.7389291

				332.12		0.7389291

				332.15		0.7389291

				332.17		0.7389291

				332.19		0.7389291

				332.21		0.7389291

				332.23		0.7389291

				332.25		0.7389291

				332.27		0.7389291

				332.29		0.7389291

				332.31		0.7389291

				332.34		0.7389291

				332.36		0.7389291

				332.38		0.7389291

				332.4		0.7389291

				332.42		0.7389291

				332.44		0.7389291

				332.46		0.7389291

				332.48		0.7389291

				332.5		0.7389291

				332.53		0.7389291

				332.55		0.7389291

				332.57		0.7389291

				332.59		0.7389291

				332.61		0.7389291

				332.63		0.7389291

				332.65		0.7389291

				332.67		0.7389291

				332.69		0.7389291

				332.72		0.7389291

				332.74		0.7389291

				332.76		0.7389291

				332.78		0.7337253

				332.8		0.7337253

				332.82		0.7337253

				332.84		0.7337253

				332.86		0.7337253

				332.88		0.7337253

				332.91		0.7337253

				332.93		0.7337253

				332.95		0.7337253

				332.97		0.7337253

				332.99		0.7337253

				333.01		0.7337253

				333.03		0.7337253

				333.05		0.7337253

				333.07		0.7337253

				333.1		0.7337253

				333.12		0.7337253

				333.14		0.7337253

				333.16		0.7337253

				333.18		0.7285216

				333.2		0.7285216

				333.22		0.7337253

				333.24		0.7337253

				333.27		0.7337253

				333.29		0.7337253

				333.31		0.7337253

				333.33		0.7285216

				333.35		0.7337253

				333.37		0.7285216

				333.39		0.7285216

				333.41		0.7285216

				333.43		0.7285216

				333.46		0.7285216

				333.48		0.7285216

				333.5		0.7285216

				333.52		0.7285216

				333.54		0.7285216

				333.56		0.7285216

				333.58		0.7285216

				333.6		0.7285216

				333.62		0.7285216

				333.65		0.7285216

				333.67		0.7285216

				333.69		0.7285216

				333.71		0.7285216

				333.73		0.7285216

				333.75		0.7285216

				333.77		0.7285216

				333.79		0.7285216

				333.81		0.7285216

				333.84		0.7285216

				333.86		0.7285216

				333.88		0.7285216

				333.9		0.7285216

				333.92		0.7285216

				333.94		0.7285216

				333.96		0.7285216

				333.98		0.7285216

				334		0.7285216

				334.03		0.7285216

				334.05		0.7285216

				334.07		0.7285216

				334.09		0.7285216

				334.11		0.7285216

				334.13		0.7285216

				334.15		0.7285216

				334.17		0.7285216

				334.19		0.7285216

				334.22		0.7285216

				334.24		0.7285216

				334.26		0.7285216

				334.28		0.7285216

				334.3		0.7285216

				334.32		0.7285216

				334.34		0.7285216

				334.36		0.7285216

				334.39		0.7285216

				334.41		0.7285216

				334.43		0.7285216

				334.45		0.7285216

				334.47		0.7285216

				334.49		0.7285216

				334.51		0.7233179

				334.53		0.7285216

				334.55		0.7285216

				334.58		0.7285216

				334.6		0.7285216

				334.62		0.7285216

				334.64		0.7285216

				334.66		0.7285216

				334.68		0.7285216

				334.7		0.7233179

				334.72		0.7233179

				334.74		0.7233179

				334.77		0.7233179

				334.79		0.7233179

				334.81		0.7233179

				334.83		0.7233179

				334.85		0.7233179

				334.87		0.7233179

				334.89		0.7233179

				334.91		0.7233179

				334.93		0.7285216

				334.96		0.7233179

				334.98		0.7285216

				335		0.7285216

				335.02		0.7233179

				335.04		0.7285216

				335.06		0.7285216

				335.08		0.7233179

				335.1		0.7233179

				335.12		0.7233179

				335.15		0.7233179

				335.17		0.7233179

				335.19		0.7233179

				335.21		0.7233179

				335.23		0.7233179

				335.25		0.7233179

				335.27		0.7233179

				335.29		0.7233179

				335.31		0.7233179

				335.34		0.7233179

				335.36		0.7233179

				335.38		0.7233179

				335.4		0.7233179

				335.42		0.7233179

				335.44		0.7233179

				335.46		0.7233179

				335.48		0.7233179

				335.51		0.7233179

				335.53		0.7233179

				335.55		0.7233179

				335.57		0.7233179

				335.59		0.7233179

				335.61		0.7233179

				335.63		0.7233179

				335.65		0.7233179

				335.67		0.7233179

				335.7		0.7233179

				335.72		0.7233179

				335.74		0.7233179

				335.76		0.7233179

				335.78		0.7233179

				335.8		0.7233179

				335.82		0.7233179

				335.84		0.7233179

				335.86		0.7233179

				335.89		0.7233179

				335.91		0.7233179

				335.93		0.7233179

				335.95		0.7233179

				335.97		0.7233179

				335.99		0.7233179

				336.01		0.7233179

				336.03		0.7233179

				336.05		0.7233179

				336.08		0.7233179

				336.1		0.7233179

				336.12		0.7233179

				336.14		0.7233179

				336.16		0.7233179

				336.18		0.7233179

				336.2		0.7233179

				336.22		0.7233179

				336.25		0.7233179

				336.27		0.7233179

				336.29		0.7233179

				336.31		0.7233179

				336.33		0.7233179

				336.35		0.7181142

				336.37		0.7233179

				336.39		0.7181142

				336.41		0.7233179

				336.44		0.7181142

				336.46		0.7181142

				336.48		0.7181142

				336.5		0.7181142

				336.52		0.7181142

				336.54		0.7181142

				336.56		0.7181142

				336.58		0.7181142

				336.6		0.7181142

				336.63		0.7181142

				336.65		0.7181142

				336.67		0.7181142

				336.69		0.7181142

				336.71		0.7181142

				336.73		0.7181142

				336.75		0.7181142

				336.77		0.7181142

				336.8		0.7181142

				336.82		0.7181142

				336.84		0.7181142

				336.86		0.7181142

				336.88		0.7181142

				336.9		0.7181142

				336.92		0.7181142

				336.94		0.7181142

				336.96		0.7181142

				336.99		0.7181142

				337.01		0.7181142

				337.03		0.7181142

				337.05		0.7181142

				337.07		0.7181142

				337.09		0.7181142

				337.11		0.7181142

				337.13		0.7181142

				337.15		0.7181142

				337.18		0.7181142

				337.2		0.7181142

				337.22		0.7181142

				337.24		0.7181142

				337.26		0.7233179

				337.28		0.7233179

				337.3		0.7233179

				337.32		0.7233179

				337.34		0.7233179

				337.37		0.7233179

				337.39		0.7233179

				337.41		0.7233179

				337.43		0.7233179

				337.45		0.7233179

				337.47		0.7233179

				337.49		0.7233179

				337.51		0.7233179

				337.54		0.7233179

				337.56		0.7233179

				337.58		0.7233179

				337.6		0.7233179

				337.62		0.7233179

				337.64		0.7233179

				337.66		0.7233179

				337.68		0.7233179

				337.7		0.7233179

				337.73		0.7233179

				337.75		0.7233179

				337.77		0.7233179

				337.79		0.7233179

				337.81		0.7233179

				337.83		0.7233179

				337.85		0.7233179

				337.87		0.7233179

				337.9		0.7233179

				337.92		0.7233179

				337.94		0.7233179

				337.96		0.7233179

				337.98		0.7233179

				338		0.7233179

				338.02		0.7233179

				338.04		0.7233179

				338.06		0.7233179

				338.09		0.7233179

				338.11		0.7233179

				338.13		0.7233179

				338.15		0.7233179

				338.17		0.7233179

				338.19		0.7233179

				338.21		0.7233179

				338.23		0.7233179

				338.26		0.7233179

				338.28		0.7233179

				338.3		0.7233179

				338.32		0.7233179

				338.34		0.7233179

				338.36		0.7233179

				338.38		0.7233179

				338.4		0.7233179

				338.42		0.7233179

				338.45		0.7233179

				338.47		0.7233179

				338.49		0.7233179

				338.51		0.7233179

				338.53		0.7233179

				338.55		0.7233179

				338.57		0.7233179

				338.59		0.7233179

				338.61		0.7233179

				338.64		0.7233179

				338.66		0.7233179

				338.68		0.7233179

				338.7		0.7233179

				338.72		0.7233179

				338.74		0.7233179

				338.76		0.7233179

				338.78		0.7233179

				338.81		0.7233179

				338.83		0.7233179

				338.85		0.7285216

				338.87		0.7233179

				338.89		0.7233179

				338.91		0.7285216

				338.93		0.7233179

				338.95		0.7233179

				338.97		0.7233179

				339		0.7285216

				339.02		0.7285216

				339.04		0.7285216

				339.06		0.7233179

				339.08		0.7285216

				339.1		0.7285216

				339.12		0.7285216

				339.14		0.7285216

				339.16		0.7285216

				339.19		0.7285216

				339.21		0.7285216

				339.23		0.7285216

				339.25		0.7285216

				339.27		0.7285216

				339.29		0.7285216

				339.31		0.7285216

				339.33		0.7285216

				339.35		0.7285216

				339.38		0.7285216

				339.4		0.7285216

				339.42		0.7233179

				339.44		0.7233179

				339.46		0.7233179

				339.48		0.7233179

				339.5		0.7233179

				339.52		0.7233179

				339.54		0.7233179

				339.57		0.7233179

				339.59		0.7233179

				339.61		0.7233179

				339.63		0.7233179

				339.65		0.7285216

				339.67		0.7233179

				339.69		0.7285216

				339.71		0.7285216

				339.74		0.7233179

				339.76		0.7285216

				339.78		0.7285216

				339.8		0.7233179

				339.82		0.7285216

				339.84		0.7233179

				339.86		0.7285216

				339.88		0.7233179

				339.9		0.7233179

				339.93		0.7233179

				339.95		0.7233179

				339.97		0.7233179

				339.99		0.7233179

				340.01		0.7233179

				340.03		0.7233179

				340.05		0.7233179

				340.07		0.7233179

				340.09		0.7233179

				340.12		0.7233179

				340.14		0.7233179

				340.16		0.7233179

				340.18		0.7233179

				340.2		0.7233179

				340.22		0.7233179

				340.24		0.7233179

				340.26		0.7233179

				340.29		0.7233179

				340.31		0.7233179

				340.33		0.7233179

				340.35		0.7233179

				340.37		0.7181142

				340.39		0.7181142

				340.41		0.7181142

				340.43		0.7181142

				340.45		0.7181142

				340.48		0.7181142

				340.5		0.7181142

				340.52		0.7181142

				340.54		0.7181142

				340.56		0.7181142

				340.58		0.7181142

				340.6		0.7181142

				340.62		0.7181142

				340.64		0.7181142

				340.67		0.7181142

				340.69		0.7181142

				340.71		0.7181142

				340.73		0.7181142

				340.75		0.7181142

				340.77		0.7181142

				340.79		0.7129104

				340.81		0.7129104

				340.84		0.7129104

				340.86		0.7129104

				340.88		0.7129104

				340.9		0.7129104

				340.92		0.7129104

				340.94		0.7129104

				340.96		0.7129104

				340.98		0.7129104

				341		0.7129104

				341.03		0.7129104

				341.05		0.7129104

				341.07		0.7129104

				341.09		0.7129104

				341.11		0.7129104

				341.13		0.7129104

				341.15		0.7129104

				341.17		0.7129104

				341.19		0.7129104

				341.22		0.7129104

				341.24		0.7129104

				341.26		0.7129104

				341.28		0.7129104

				341.3		0.7129104

				341.32		0.7129104

				341.34		0.7129104

				341.36		0.7129104

				341.38		0.7129104

				341.41		0.7129104

				341.43		0.7077067

				341.45		0.7077067

				341.47		0.7077067

				341.49		0.7077067

				341.51		0.7077067

				341.53		0.7129104

				341.55		0.7129104

				341.57		0.7077067

				341.6		0.7077067

				341.62		0.7077067

				341.64		0.7077067

				341.66		0.7077067

				341.68		0.7077067

				341.7		0.7077067

				341.72		0.7077067

				341.74		0.7077067

				341.77		0.7077067

				341.79		0.7077067

				341.81		0.7077067

				341.83		0.7077067

				341.85		0.7077067

				341.87		0.7077067

				341.89		0.7077067

				341.91		0.7077067

				341.93		0.7077067

				341.96		0.702503

				341.98		0.7077067

				342		0.7077067

				342.02		0.7077067

				342.04		0.7077067

				342.06		0.7077067

				342.08		0.7077067

				342.1		0.7077067

				342.12		0.702503

				342.15		0.7077067

				342.17		0.7077067

				342.19		0.702503

				342.21		0.702503

				342.23		0.702503

				342.25		0.702503

				342.27		0.702503

				342.29		0.702503

				342.31		0.702503

				342.34		0.702503

				342.36		0.702503

				342.38		0.702503

				342.4		0.702503

				342.42		0.702503

				342.44		0.702503

				342.46		0.702503

				342.48		0.702503

				342.51		0.702503

				342.53		0.702503

				342.55		0.702503

				342.57		0.702503

				342.59		0.702503

				342.61		0.702503

				342.63		0.702503

				342.65		0.702503

				342.67		0.7077067

				342.7		0.7077067

				342.72		0.702503

				342.74		0.702503

				342.76		0.7077067

				342.78		0.7077067

				342.8		0.7077067

				342.82		0.7077067

				342.84		0.7077067

				342.86		0.702503

				342.89		0.7077067

				342.91		0.7077067

				342.93		0.7077067

				342.95		0.702503

				342.97		0.7077067

				342.99		0.702503

				343.01		0.702503

				343.03		0.702503

				343.06		0.702503

				343.08		0.702503

				343.1		0.702503

				343.12		0.702503

				343.14		0.702503

				343.16		0.702503

				343.18		0.702503

				343.2		0.702503

				343.22		0.702503

				343.25		0.702503

				343.27		0.702503

				343.29		0.702503

				343.31		0.702503

				343.33		0.702503

				343.35		0.702503

				343.37		0.702503

				343.39		0.702503

				343.41		0.702503

				343.44		0.702503

				343.46		0.702503

				343.48		0.702503

				343.5		0.702503

				343.52		0.702503

				343.54		0.702503

				343.56		0.702503

				343.58		0.702503

				343.61		0.702503

				343.63		0.702503

				343.65		0.702503

				343.67		0.702503

				343.69		0.702503

				343.71		0.702503

				343.73		0.702503

				343.75		0.702503

				343.77		0.702503

				343.8		0.702503

				343.82		0.702503

				343.84		0.702503

				343.86		0.702503

				343.88		0.702503

				343.9		0.702503

				343.92		0.702503

				343.94		0.702503

				343.96		0.702503

				343.99		0.7077067

				344.01		0.7077067

				344.03		0.702503

				344.05		0.7077067

				344.07		0.7077067

				344.09		0.7077067

				344.11		0.7077067

				344.13		0.7077067

				344.16		0.7077067

				344.18		0.7077067

				344.2		0.7077067

				344.22		0.7077067

				344.24		0.7077067

				344.26		0.7077067

				344.28		0.7077067

				344.3		0.7077067

				344.32		0.7077067

				344.35		0.7077067

				344.37		0.7077067

				344.39		0.7077067

				344.41		0.7077067

				344.43		0.7077067

				344.45		0.7077067

				344.47		0.7077067

				344.49		0.7077067

				344.52		0.7077067

				344.54		0.7077067

				344.56		0.7077067

				344.58		0.7077067

				344.6		0.7077067

				344.62		0.7077067

				344.64		0.7077067

				344.66		0.7077067

				344.68		0.7077067

				344.71		0.7077067

				344.73		0.7077067

				344.75		0.7077067

				344.77		0.7077067

				344.79		0.7077067

				344.81		0.7077067

				344.83		0.7077067

				344.85		0.7077067

				344.87		0.7077067

				344.9		0.7077067

				344.92		0.7077067

				344.94		0.7077067

				344.96		0.702503

				344.98		0.7077067

				345		0.7077067

				345.02		0.7077067

				345.04		0.7077067

				345.07		0.7077067

				345.09		0.7077067

				345.11		0.7077067

				345.13		0.7077067

				345.15		0.7077067

				345.17		0.7077067

				345.19		0.7077067

				345.21		0.7077067

				345.23		0.7077067

				345.26		0.7077067

				345.28		0.7077067

				345.3		0.7077067

				345.32		0.7077067

				345.34		0.7077067

				345.36		0.7077067

				345.38		0.7077067

				345.4		0.702503

				345.42		0.702503

				345.45		0.702503

				345.47		0.702503

				345.49		0.702503

				345.51		0.702503

				345.53		0.702503

				345.55		0.702503

				345.57		0.702503

				345.59		0.702503

				345.61		0.702503

				345.64		0.702503

				345.66		0.702503

				345.68		0.702503

				345.7		0.702503

				345.72		0.702503

				345.74		0.702503

				345.76		0.702503

				345.78		0.702503

				345.81		0.702503

				345.83		0.702503

				345.85		0.6972993

				345.87		0.6972993

				345.89		0.6972993

				345.91		0.6972993

				345.93		0.6972993

				345.95		0.6972993

				345.97		0.702503

				346		0.6972993

				346.02		0.702503

				346.04		0.6972993

				346.06		0.6972993

				346.08		0.6972993

				346.1		0.6972993

				346.12		0.6972993

				346.14		0.6972993

				346.17		0.6972993

				346.19		0.6972993

				346.21		0.6972993

				346.23		0.6972993

				346.25		0.6972993

				346.27		0.6972993

				346.29		0.6972993

				346.31		0.6972993

				346.33		0.6972993

				346.36		0.6972993

				346.38		0.6972993

				346.4		0.6972993

				346.42		0.6972993

				346.44		0.6972993

				346.46		0.6972993

				346.48		0.6972993

				346.5		0.6972993

				346.53		0.6972993

				346.55		0.6972993

				346.57		0.6972993

				346.59		0.6972993

				346.61		0.6972993

				346.63		0.6972993

				346.65		0.6972993

				346.67		0.6972993

				346.69		0.6972993

				346.72		0.6972993

				346.74		0.6972993

				346.76		0.6972993

				346.78		0.6972993

				346.8		0.6972993

				346.82		0.6972993

				346.84		0.6972993

				346.86		0.6972993

				346.89		0.6972993

				346.91		0.6972993

				346.93		0.6972993

				346.95		0.6972993

				346.97		0.6972993

				346.99		0.6972993

				347.01		0.6972993

				347.03		0.6972993

				347.05		0.6972993

				347.08		0.6972993

				347.1		0.6972993

				347.12		0.6972993

				347.14		0.6972993

				347.16		0.6972993

				347.18		0.6972993

				347.2		0.6972993

				347.22		0.6972993

				347.25		0.6972993

				347.27		0.6972993

				347.29		0.6920955

				347.31		0.6920955

				347.33		0.6920955

				347.35		0.6920955

				347.37		0.6920955

				347.39		0.6920955

				347.41		0.6920955

				347.44		0.6920955

				347.46		0.6920955

				347.48		0.6920955

				347.5		0.6920955

				347.52		0.6920955

				347.54		0.6920955

				347.56		0.6920955

				347.58		0.6920955

				347.61		0.6920955

				347.63		0.6920955

				347.65		0.6920955

				347.67		0.6920955

				347.69		0.6920955

				347.71		0.6920955

				347.73		0.6920955

				347.75		0.6920955

				347.77		0.6920955

				347.8		0.6920955

				347.82		0.6920955

				347.84		0.6920955

				347.86		0.6920955

				347.88		0.6920955

				347.9		0.6920955

				347.92		0.6920955

				347.94		0.6920955

				347.97		0.6920955

				347.99		0.6920955

				348.01		0.6920955

				348.03		0.6920955

				348.05		0.6920955

				348.07		0.6920955

				348.09		0.6920955

				348.11		0.6920955

				348.14		0.6920955

				348.16		0.6920955

				348.18		0.6920955

				348.2		0.6920955

				348.22		0.6920955

				348.24		0.6920955

				348.26		0.6920955

				348.28		0.6920955

				348.3		0.6920955

				348.33		0.6920955

				348.35		0.6920955

				348.37		0.6920955

				348.39		0.6920955

				348.41		0.6920955

				348.43		0.6920955

				348.45		0.6920955

				348.47		0.6920955

				348.5		0.6920955

				348.52		0.6920955

				348.54		0.6920955

				348.56		0.6920955

				348.58		0.6920955

				348.6		0.6920955

				348.62		0.6920955

				348.64		0.6920955

				348.66		0.6920955

				348.69		0.6920955

				348.71		0.6920955

				348.73		0.6920955

				348.75		0.6920955

				348.77		0.6920955

				348.79		0.6920955

				348.81		0.6920955

				348.83		0.6920955

				348.86		0.6920955

				348.88		0.6920955

				348.9		0.6868918

				348.92		0.6868918

				348.94		0.6868918

				348.96		0.6868918

				348.98		0.6868918

				349		0.6868918

				349.02		0.6868918

				349.05		0.6868918

				349.07		0.6868918

				349.09		0.6868918

				349.11		0.6868918

				349.13		0.6868918

				349.15		0.6868918

				349.17		0.6868918

				349.19		0.6868918

				349.22		0.6868918

				349.24		0.6868918

				349.26		0.6868918

				349.28		0.6868918

				349.3		0.6868918

				349.32		0.6868918

				349.34		0.6868918

				349.36		0.6868918

				349.39		0.6868918

				349.41		0.6868918

				349.43		0.6868918

				349.45		0.6868918

				349.47		0.6868918

				349.49		0.6868918

				349.51		0.6868918

				349.54		0.6868918

				349.56		0.6868918

				349.58		0.6868918

				349.6		0.6868918

				349.62		0.6868918

				349.64		0.6868918

				349.66		0.6868918

				349.69		0.6868918

				349.71		0.6868918

				349.73		0.6868918

				349.75		0.6868918

				349.77		0.6868918

				349.79		0.6868918

				349.81		0.6868918

				349.84		0.6868918

				349.86		0.6868918

				349.88		0.6868918

				349.9		0.6868918

				349.92		0.6868918

				349.94		0.6868918

				349.96		0.6868918

				349.99		0.6868918

				350.01		0.6868918

				350.03		0.6816881

				350.05		0.6816881

				350.07		0.6816881

				350.09		0.6816881

				350.11		0.6816881

				350.13		0.6816881

				350.16		0.6816881

				350.18		0.6816881

				350.2		0.6816881

				350.22		0.6816881

				350.24		0.6816881

				350.26		0.6816881

				350.28		0.6816881

				350.31		0.6816881

				350.33		0.6816881

				350.35		0.6816881

				350.37		0.6816881

				350.39		0.6816881

				350.41		0.6816881

				350.43		0.6816881

				350.45		0.6816881

				350.48		0.6816881

				350.5		0.6816881

				350.52		0.6816881

				350.54		0.6816881

				350.56		0.6816881

				350.58		0.6816881

				350.6		0.6764844

				350.62		0.6764844

				350.65		0.6764844

				350.67		0.6764844

				350.69		0.6764844

				350.71		0.6764844

				350.73		0.6764844

				350.75		0.6764844

				350.77		0.6764844

				350.79		0.6764844

				350.81		0.6764844

				350.84		0.6764844

				350.86		0.6764844

				350.88		0.6764844

				350.9		0.6764844

				350.92		0.6764844

				350.94		0.6764844

				350.96		0.6764844

				350.98		0.6764844

				351		0.6764844

				351.03		0.6764844

				351.05		0.6712806

				351.07		0.6712806

				351.09		0.6712806

				351.11		0.6712806

				351.13		0.6712806

				351.15		0.6712806

				351.17		0.6764844

				351.2		0.6712806

				351.22		0.6764844

				351.24		0.6712806

				351.26		0.6712806

				351.28		0.6712806

				351.3		0.6712806

				351.32		0.6712806

				351.34		0.6712806

				351.37		0.6764844

				351.39		0.6712806

				351.41		0.6712806

				351.43		0.6712806

				351.45		0.6764844

				351.47		0.6712806

				351.49		0.6712806

				351.51		0.6712806

				351.53		0.6712806

				351.56		0.6712806

				351.58		0.6712806

				351.6		0.6712806

				351.62		0.6712806

				351.64		0.6764844

				351.66		0.6712806

				351.68		0.6712806

				351.7		0.6712806

				351.73		0.6712806

				351.75		0.6764844

				351.77		0.6764844

				351.79		0.6764844

				351.81		0.6764844

				351.83		0.6764844

				351.85		0.6712806

				351.87		0.6764844

				351.9		0.6712806

				351.92		0.6712806

				351.94		0.6712806

				351.96		0.6764844

				351.98		0.6712806

				352		0.6712806

				352.02		0.6712806

				352.04		0.6712806

				352.07		0.6712806

				352.09		0.6712806

				352.11		0.6712806

				352.13		0.6712806

				352.15		0.6712806

				352.17		0.6712806

				352.19		0.6712806

				352.21		0.6712806

				352.23		0.6712806

				352.26		0.6764844

				352.28		0.6712806

				352.3		0.6764844

				352.32		0.6712806

				352.34		0.6764844

				352.36		0.6712806

				352.38		0.6764844

				352.4		0.6764844

				352.43		0.6712806

				352.45		0.6712806

				352.47		0.6712806

				352.49		0.6712806

				352.51		0.6712806

				352.53		0.6712806

				352.55		0.6712806

				352.57		0.6712806

				352.6		0.6712806

				352.62		0.6712806

				352.64		0.6712806

				352.66		0.6712806

				352.68		0.6712806

				352.7		0.6712806

				352.72		0.6712806

				352.74		0.6712806

				352.77		0.6712806

				352.79		0.6712806

				352.81		0.6712806

				352.83		0.6712806

				352.85		0.6712806

				352.87		0.6712806

				352.89		0.6712806

				352.91		0.6712806

				352.94		0.6712806

				352.96		0.6712806

				352.98		0.6712806

				353		0.6712806

				353.02		0.6712806

				353.04		0.6712806

				353.06		0.6712806

				353.08		0.6712806

				353.11		0.6764844

				353.13		0.6712806

				353.15		0.6712806

				353.17		0.6712806

				353.19		0.6712806

				353.21		0.6712806

				353.23		0.6712806

				353.25		0.6764844

				353.28		0.6712806

				353.3		0.6712806

				353.32		0.6712806

				353.34		0.6764844

				353.36		0.6764844

				353.38		0.6712806

				353.4		0.6712806

				353.42		0.6712806

				353.45		0.6712806

				353.47		0.6712806

				353.49		0.6712806

				353.51		0.6712806

				353.53		0.6712806

				353.55		0.6712806

				353.57		0.6712806

				353.59		0.6712806

				353.62		0.6712806

				353.64		0.6712806

				353.66		0.6712806

				353.68		0.6712806

				353.7		0.6712806

				353.72		0.6712806

				353.74		0.6712806

				353.76		0.6712806

				353.79		0.6712806

				353.81		0.6660769

				353.83		0.6712806

				353.85		0.6660769

				353.87		0.6712806

				353.89		0.6712806

				353.91		0.6660769

				353.93		0.6712806

				353.96		0.6660769

				353.98		0.6660769

				354		0.6660769

				354.02		0.6660769

				354.04		0.6660769

				354.06		0.6660769

				354.08		0.6660769

				354.1		0.6660769

				354.13		0.6660769

				354.15		0.6660769

				354.17		0.6660769

				354.19		0.6660769

				354.21		0.6660769

				354.23		0.6660769

				354.25		0.6660769

				354.27		0.6660769

				354.3		0.6660769

				354.32		0.6660769

				354.34		0.6660769

				354.36		0.6660769

				354.38		0.6660769

				354.4		0.6660769

				354.42		0.6660769

				354.44		0.6660769

				354.47		0.6660769

				354.49		0.6660769

				354.51		0.6660769

				354.53		0.6660769

				354.55		0.6660769

				354.57		0.6660769

				354.59		0.6660769

				354.61		0.6660769

				354.64		0.6660769

				354.66		0.6660769

				354.68		0.6660769

				354.7		0.6660769

				354.72		0.6660769

				354.74		0.6660769

				354.76		0.6660769

				354.78		0.6660769

				354.81		0.6660769

				354.83		0.6660769

				354.85		0.6660769

				354.87		0.6660769

				354.89		0.6660769

				354.91		0.6660769

				354.93		0.6660769

				354.95		0.6660769

				354.98		0.6660769

				355		0.6660769

				355.02		0.6660769

				355.04		0.6660769

				355.06		0.6660769

				355.08		0.6660769

				355.1		0.6660769

				355.12		0.6660769

				355.15		0.6660769

				355.17		0.6660769

				355.19		0.6660769

				355.21		0.6660769

				355.23		0.6660769

				355.25		0.6660769

				355.27		0.6660769

				355.29		0.6660769

				355.32		0.6660769

				355.34		0.6660769

				355.36		0.6660769

				355.38		0.6660769

				355.4		0.6660769

				355.42		0.6660769

				355.44		0.6660769

				355.46		0.6660769

				355.49		0.6660769

				355.51		0.6660769

				355.53		0.6660769

				355.55		0.6660769

				355.57		0.6660769

				355.59		0.6660769

				355.61		0.6660769

				355.63		0.6660769

				355.66		0.6660769

				355.68		0.6660769

				355.7		0.6660769

				355.72		0.6660769

				355.74		0.6660769

				355.76		0.6660769

				355.78		0.6660769

				355.81		0.6660769

				355.83		0.6660769

				355.85		0.6608732

				355.87		0.6660769

				355.89		0.6660769

				355.91		0.6660769

				355.93		0.6608732

				355.95		0.6660769

				355.98		0.6660769

				356		0.6660769

				356.02		0.6660769

				356.04		0.6660769

				356.06		0.6660769

				356.08		0.6660769

				356.1		0.6660769

				356.12		0.6660769

				356.15		0.6660769

				356.17		0.6660769

				356.19		0.6660769

				356.21		0.6660769

				356.23		0.6660769

				356.25		0.6660769

				356.27		0.6660769

				356.29		0.6660769

				356.32		0.6660769

				356.34		0.6660769

				356.36		0.6660769

				356.38		0.6712806

				356.4		0.6660769

				356.42		0.6712806

				356.44		0.6712806

				356.46		0.6712806

				356.49		0.6712806

				356.51		0.6712806

				356.53		0.6712806

				356.55		0.6660769

				356.57		0.6712806

				356.59		0.6660769

				356.61		0.6660769

				356.63		0.6660769

				356.66		0.6660769

				356.68		0.6660769

				356.7		0.6660769

				356.72		0.6660769

				356.74		0.6660769

				356.76		0.6660769

				356.78		0.6712806

				356.8		0.6712806

				356.83		0.6712806

				356.85		0.6712806

				356.87		0.6712806

				356.89		0.6712806

				356.91		0.6712806

				356.93		0.6712806

				356.95		0.6712806

				356.97		0.6712806

				357		0.6712806

				357.02		0.6712806

				357.04		0.6712806

				357.06		0.6712806

				357.08		0.6712806

				357.1		0.6712806

				357.12		0.6712806

				357.14		0.6660769

				357.17		0.6712806

				357.19		0.6712806

				357.21		0.6712806

				357.23		0.6712806

				357.25		0.6712806

				357.27		0.6712806

				357.29		0.6712806

				357.31		0.6712806

				357.34		0.6712806

				357.36		0.6712806

				357.38		0.6712806

				357.4		0.6712806

				357.42		0.6712806

				357.44		0.6712806

				357.46		0.6712806

				357.48		0.6712806

				357.51		0.6712806

				357.53		0.6712806

				357.55		0.6712806

				357.57		0.6712806

				357.59		0.6712806

				357.61		0.6712806

				357.63		0.6712806

				357.65		0.6712806

				357.68		0.6712806

				357.7		0.6712806

				357.72		0.6712806

				357.74		0.6712806

				357.76		0.6712806

				357.78		0.6712806

				357.8		0.6712806

				357.82		0.6712806

				357.85		0.6712806

				357.87		0.6712806

				357.89		0.6712806

				357.91		0.6712806

				357.93		0.6712806

				357.95		0.6764844

				357.97		0.6764844

				357.99		0.6764844

				358.02		0.6764844

				358.04		0.6764844

				358.06		0.6764844

				358.08		0.6764844

				358.1		0.6764844

				358.12		0.6764844

				358.14		0.6764844

				358.16		0.6764844

				358.19		0.6764844

				358.21		0.6712806

				358.23		0.6712806

				358.25		0.6712806

				358.27		0.6712806

				358.29		0.6712806

				358.31		0.6712806

				358.33		0.6764844

				358.36		0.6712806

				358.38		0.6764844

				358.4		0.6764844

				358.42		0.6712806

				358.44		0.6764844

				358.46		0.6764844

				358.48		0.6764844

				358.5		0.6764844

				358.53		0.6764844

				358.55		0.6712806

				358.57		0.6712806

				358.59		0.6712806

				358.61		0.6712806

				358.63		0.6712806

				358.65		0.6712806

				358.67		0.6712806

				358.7		0.6712806

				358.72		0.6712806

				358.74		0.6712806

				358.76		0.6712806

				358.78		0.6712806

				358.8		0.6712806

				358.82		0.6712806

				358.84		0.6712806

				358.87		0.6712806

				358.89		0.6712806

				358.91		0.6712806

				358.93		0.6712806

				358.95		0.6712806

				358.97		0.6712806

				358.99		0.6712806

				359.01		0.6712806

				359.04		0.6712806

				359.06		0.6712806

				359.08		0.6712806

				359.1		0.6660769

				359.12		0.6712806

				359.14		0.6660769

				359.16		0.6660769

				359.18		0.6660769

				359.21		0.6660769

				359.23		0.6660769

				359.25		0.6712806

				359.27		0.6712806

				359.29		0.6712806

				359.31		0.6712806

				359.33		0.6712806

				359.35		0.6712806

				359.38		0.6712806

				359.4		0.6712806

				359.42		0.6712806

				359.44		0.6712806

				359.46		0.6712806

				359.48		0.6712806

				359.5		0.6712806

				359.52		0.6712806

				359.55		0.6712806

				359.57		0.6712806

				359.59		0.6712806

				359.61		0.6712806

				359.63		0.6660769

				359.65		0.6712806

				359.67		0.6712806

				359.69		0.6712806

				359.72		0.6712806

				359.74		0.6712806

				359.76		0.6712806

				359.78		0.6712806

				359.8		0.6712806

				359.82		0.6712806

				359.84		0.6712806

				359.86		0.6712806

				359.89		0.6712806

				359.91		0.6712806

				359.93		0.6712806

				359.95		0.6712806

				359.97		0.6712806

				359.99		0.6712806

				360.01		0.6712806

				360.03		0.6712806

				360.06		0.6712806

				360.08		0.6712806

				360.1		0.6712806

				360.12		0.6712806

				360.14		0.6712806

				360.16		0.6712806

				360.18		0.6712806

				360.2		0.6712806

				360.23		0.6712806

				360.25		0.6712806

				360.27		0.6712806

				360.29		0.6712806

				360.31		0.6712806

				360.33		0.6712806

				360.35		0.6712806

				360.37		0.6712806

				360.4		0.6712806

				360.42		0.6712806

				360.44		0.6712806

				360.46		0.6712806

				360.48		0.6712806

				360.5		0.6712806

				360.52		0.6712806

				360.54		0.6712806

				360.57		0.6712806

				360.59		0.6712806

				360.61		0.6712806

				360.63		0.6712806

				360.65		0.6712806

				360.67		0.6712806

				360.69		0.6712806

				360.71		0.6712806

				360.74		0.6712806

				360.76		0.6712806

				360.78		0.6712806

				360.8		0.6712806

				360.82		0.6712806

				360.84		0.6712806

				360.86		0.6712806

				360.88		0.6712806

				360.91		0.6712806

				360.93		0.6712806

				360.95		0.6712806

				360.97		0.6712806

				360.99		0.6712806

				361.01		0.6712806

				361.03		0.6712806

				361.05		0.6712806

				361.07		0.6712806

				361.1		0.6712806

				361.12		0.6712806

				361.14		0.6712806

				361.16		0.6712806

				361.18		0.6712806

				361.2		0.6764844

				361.22		0.6764844

				361.24		0.6764844

				361.27		0.6764844

				361.29		0.6764844

				361.31		0.6764844

				361.33		0.6764844

				361.35		0.6764844

				361.37		0.6764844

				361.39		0.6764844

				361.41		0.6764844

				361.44		0.6764844

				361.46		0.6764844

				361.48		0.6764844

				361.5		0.6764844

				361.52		0.6764844

				361.54		0.6764844

				361.56		0.6764844

				361.58		0.6764844

				361.61		0.6764844

				361.63		0.6764844

				361.65		0.6764844

				361.67		0.6764844

				361.69		0.6764844

				361.71		0.6764844

				361.73		0.6764844

				361.75		0.6764844

				361.78		0.6764844

				361.8		0.6764844

				361.82		0.6764844

				361.84		0.6764844

				361.86		0.6764844

				361.88		0.6764844

				361.9		0.6764844

				361.92		0.6764844

				361.95		0.6764844

				361.97		0.6764844

				361.99		0.6764844

				362.01		0.6764844

				362.03		0.6764844

				362.05		0.6764844

				362.07		0.6764844

				362.09		0.6764844

				362.12		0.6764844

				362.14		0.6712806

				362.16		0.6712806

				362.18		0.6764844

				362.2		0.6712806

				362.22		0.6712806

				362.24		0.6764844

				362.26		0.6764844

				362.29		0.6764844

				362.31		0.6764844

				362.33		0.6764844

				362.35		0.6764844

				362.37		0.6712806

				362.39		0.6712806

				362.41		0.6764844

				362.43		0.6712806

				362.46		0.6712806

				362.48		0.6712806

				362.5		0.6712806

				362.52		0.6712806

				362.54		0.6712806

				362.56		0.6712806

				362.58		0.6712806

				362.6		0.6712806

				362.63		0.6712806

				362.65		0.6712806

				362.67		0.6712806

				362.69		0.6712806

				362.71		0.6712806

				362.73		0.6712806

				362.75		0.6712806

				362.77		0.6712806

				362.79		0.6712806

				362.82		0.6712806

				362.84		0.6712806

				362.86		0.6712806

				362.88		0.6712806

				362.9		0.6712806

				362.92		0.6712806

				362.94		0.6712806

				362.96		0.6712806

				362.99		0.6712806

				363.01		0.6712806

				363.03		0.6712806

				363.05		0.6712806

				363.07		0.6660769

				363.09		0.6712806

				363.11		0.6660769

				363.13		0.6712806

				363.16		0.6660769

				363.18		0.6660769

				363.2		0.6660769

				363.22		0.6660769

				363.24		0.6660769

				363.26		0.6660769

				363.28		0.6660769

				363.3		0.6660769

				363.33		0.6660769

				363.35		0.6660769

				363.37		0.6660769

				363.39		0.6660769

				363.41		0.6660769

				363.43		0.6660769

				363.45		0.6660769

				363.47		0.6660769

				363.5		0.6660769

				363.52		0.6660769

				363.54		0.6660769

				363.56		0.6660769

				363.58		0.6660769

				363.6		0.6660769

				363.62		0.6660769

				363.64		0.6660769

				363.67		0.6660769

				363.69		0.6660769

				363.71		0.6660769

				363.73		0.6660769

				363.75		0.6660769

				363.77		0.6660769

				363.79		0.6660769

				363.81		0.6660769

				363.83		0.6660769

				363.86		0.6660769

				363.88		0.6660769

				363.9		0.6660769

				363.92		0.6660769

				363.94		0.6660769

				363.96		0.6660769

				363.98		0.6660769

				364		0.6660769

				364.03		0.6660769

				364.05		0.6660769

				364.07		0.6660769

				364.09		0.6608732

				364.11		0.6608732

				364.13		0.6608732

				364.15		0.6608732

				364.17		0.6608732

				364.2		0.6608732

				364.22		0.6608732

				364.24		0.6608732

				364.26		0.6608732

				364.28		0.6608732

				364.3		0.6608732

				364.32		0.6608732

				364.34		0.6608732

				364.37		0.6608732

				364.39		0.6608732

				364.41		0.6608732

				364.43		0.6608732

				364.45		0.6608732

				364.47		0.6608732

				364.49		0.6608732

				364.51		0.6608732

				364.54		0.6608732

				364.56		0.6608732

				364.58		0.6608732

				364.6		0.6608732

				364.62		0.6608732

				364.64		0.6608732

				364.66		0.6608732

				364.68		0.6608732

				364.71		0.6608732

				364.73		0.6608732

				364.75		0.6608732

				364.77		0.6608732

				364.79		0.6608732

				364.81		0.6608732

				364.83		0.6608732

				364.85		0.6608732

				364.88		0.6608732

				364.9		0.6608732

				364.92		0.6608732

				364.94		0.6608732

				364.96		0.6556695

				364.98		0.6608732

				365		0.6608732

				365.02		0.6608732

				365.05		0.6608732

				365.07		0.6608732

				365.09		0.6608732

				365.11		0.6608732

				365.13		0.6608732

				365.15		0.6608732

				365.17		0.6556695

				365.19		0.6608732

				365.22		0.6608732

				365.24		0.6608732

				365.26		0.6608732

				365.28		0.6608732

				365.3		0.6608732

				365.32		0.6608732

				365.34		0.6608732

				365.36		0.6608732

				365.39		0.6608732

				365.41		0.6608732

				365.43		0.6608732

				365.45		0.6608732

				365.47		0.6556695

				365.49		0.6556695

				365.51		0.6608732

				365.53		0.6556695

				365.56		0.6608732

				365.58		0.6608732

				365.6		0.6608732

				365.62		0.6608732

				365.64		0.6556695

				365.66		0.6556695

				365.68		0.6608732

				365.7		0.6608732

				365.73		0.6556695

				365.75		0.6608732

				365.77		0.6556695

				365.79		0.6556695

				365.81		0.6556695

				365.83		0.6556695

				365.85		0.6556695

				365.87		0.6556695

				365.9		0.6556695

				365.92		0.6556695

				365.94		0.6556695

				365.96		0.6556695

				365.98		0.6556695

				366		0.6556695

				366.02		0.6556695

				366.04		0.6556695

				366.07		0.6556695

				366.09		0.6556695

				366.11		0.6556695

				366.13		0.6556695

				366.15		0.6556695

				366.17		0.6556695

				366.19		0.6556695

				366.21		0.6556695

				366.24		0.6556695

				366.26		0.6556695

				366.28		0.6556695

				366.3		0.6556695

				366.32		0.6556695

				366.34		0.6556695

				366.36		0.6556695

				366.38		0.6556695

				366.41		0.6556695

				366.43		0.6556695

				366.45		0.6556695

				366.47		0.6556695

				366.49		0.6504657

				366.51		0.6504657

				366.53		0.6556695

				366.55		0.6504657

				366.58		0.6504657

				366.6		0.6556695

				366.62		0.6556695

				366.64		0.6556695

				366.66		0.6556695

				366.68		0.6556695

				366.7		0.6504657

				366.72		0.6504657

				366.75		0.6504657

				366.77		0.6504657

				366.79		0.6504657

				366.81		0.6504657

				366.83		0.6504657

				366.85		0.6504657

				366.87		0.6504657

				366.89		0.6504657

				366.92		0.6504657

				366.94		0.6504657

				366.96		0.6504657

				366.98		0.6504657

				367		0.6504657

				367.02		0.6504657

				367.04		0.6504657

				367.06		0.6504657

				367.09		0.6504657

				367.11		0.6504657

				367.13		0.6504657

				367.15		0.6504657

				367.17		0.6504657

				367.19		0.6504657

				367.21		0.6504657

				367.23		0.6504657

				367.26		0.6504657

				367.28		0.6504657

				367.3		0.6504657

				367.32		0.6504657

				367.34		0.6504657

				367.36		0.6504657

				367.38		0.645262

				367.4		0.6504657

				367.43		0.645262

				367.45		0.645262

				367.47		0.645262

				367.49		0.645262

				367.51		0.645262

				367.53		0.645262

				367.55		0.645262

				367.57		0.645262

				367.6		0.645262

				367.62		0.645262

				367.64		0.645262

				367.66		0.645262

				367.68		0.645262

				367.7		0.645262

				367.72		0.645262

				367.74		0.645262

				367.77		0.645262

				367.79		0.645262

				367.81		0.645262

				367.83		0.645262

				367.85		0.645262

				367.87		0.645262

				367.89		0.645262

				367.91		0.645262

				367.94		0.645262

				367.96		0.645262

				367.98		0.645262

				368		0.645262

				368.02		0.645262

				368.04		0.645262

				368.06		0.645262

				368.08		0.645262

				368.11		0.645262

				368.13		0.645262

				368.15		0.645262

				368.17		0.645262

				368.19		0.645262

				368.21		0.645262

				368.23		0.645262

				368.25		0.645262

				368.28		0.645262

				368.3		0.645262

				368.32		0.645262

				368.34		0.645262

				368.36		0.645262

				368.38		0.645262

				368.4		0.645262

				368.42		0.645262

				368.45		0.645262

				368.47		0.645262

				368.49		0.645262

				368.51		0.645262

				368.53		0.645262

				368.55		0.645262

				368.57		0.6504657

				368.59		0.6504657

				368.62		0.6504657

				368.64		0.6504657

				368.66		0.6504657

				368.68		0.6504657

				368.7		0.6504657

				368.72		0.6504657

				368.74		0.6504657

				368.76		0.6504657

				368.79		0.6504657

				368.81		0.6504657

				368.83		0.6504657

				368.85		0.6504657

				368.87		0.6504657

				368.89		0.6504657

				368.91		0.6504657

				368.93		0.6504657

				368.96		0.6504657

				368.98		0.6504657

				369		0.6504657

				369.02		0.6504657

				369.04		0.6504657

				369.06		0.6504657

				369.08		0.6504657

				369.1		0.6504657

				369.13		0.6556695

				369.15		0.6504657

				369.17		0.6504657

				369.19		0.6504657

				369.21		0.6556695

				369.23		0.6504657

				369.25		0.6504657

				369.27		0.6504657

				369.3		0.6556695

				369.32		0.6504657

				369.34		0.6504657

				369.36		0.6504657

				369.38		0.6504657

				369.4		0.6504657

				369.42		0.6556695

				369.45		0.6556695

				369.47		0.6504657

				369.49		0.6556695

				369.51		0.6556695

				369.53		0.6556695

				369.55		0.6556695

				369.57		0.6556695

				369.59		0.6556695

				369.62		0.6556695

				369.64		0.6556695

				369.66		0.6556695

				369.68		0.6556695

				369.7		0.6556695

				369.72		0.6556695

				369.74		0.6556695

				369.76		0.6556695

				369.79		0.6556695

				369.81		0.6556695

				369.83		0.6556695

				369.85		0.6556695

				369.87		0.6556695

				369.89		0.6556695

				369.91		0.6556695

				369.93		0.6556695

				369.96		0.6556695

				369.98		0.6556695

				370		0.6556695

				370.02		0.6556695

				370.04		0.6556695

				370.06		0.6556695

				370.08		0.6556695

				370.1		0.6556695

				370.13		0.6556695

				370.15		0.6556695

				370.17		0.6556695

				370.19		0.6556695

				370.21		0.6556695

				370.23		0.6556695

				370.25		0.6556695

				370.27		0.6556695

				370.3		0.6556695

				370.32		0.6556695

				370.34		0.6556695

				370.36		0.6556695

				370.38		0.6556695

				370.4		0.6556695

				370.42		0.6556695

				370.44		0.6556695

				370.47		0.6556695

				370.49		0.6556695

				370.51		0.6556695

				370.53		0.6556695

				370.55		0.6556695

				370.57		0.6556695

				370.59		0.6556695

				370.61		0.6556695

				370.64		0.6556695

				370.66		0.6556695

				370.68		0.6556695

				370.7		0.6556695

				370.72		0.6556695

				370.74		0.6556695

				370.76		0.6504657

				370.78		0.6504657

				370.81		0.6504657

				370.83		0.6504657

				370.85		0.6504657

				370.87		0.6504657

				370.89		0.6504657

				370.91		0.6504657

				370.93		0.6504657

				370.95		0.6504657

				370.98		0.6504657

				371		0.6504657

				371.02		0.6504657

				371.04		0.6504657

				371.06		0.6556695

				371.08		0.6556695

				371.1		0.6556695

				371.12		0.6556695

				371.15		0.6556695

				371.17		0.6556695

				371.19		0.6504657

				371.21		0.6556695

				371.23		0.6504657

				371.25		0.6556695

				371.27		0.6556695

				371.29		0.6556695

				371.32		0.6504657

				371.34		0.6504657

				371.36		0.6556695

				371.38		0.6504657

				371.4		0.6504657

				371.42		0.6556695

				371.44		0.6504657

				371.46		0.6504657

				371.49		0.6504657

				371.51		0.6556695

				371.53		0.6504657

				371.55		0.6556695

				371.57		0.6556695

				371.59		0.6556695

				371.61		0.6504657

				371.63		0.6556695

				371.66		0.6556695

				371.68		0.6556695

				371.7		0.6556695

				371.72		0.6556695

				371.74		0.6556695

				371.76		0.6556695

				371.78		0.6556695

				371.8		0.6556695

				371.83		0.6556695

				371.85		0.6556695

				371.87		0.6556695

				371.89		0.6556695

				371.91		0.6556695

				371.93		0.6556695

				371.95		0.6556695

				371.97		0.6556695

				372		0.6556695

				372.02		0.6556695

				372.04		0.6556695

				372.06		0.6556695

				372.08		0.6556695

				372.1		0.6556695

				372.12		0.6556695

				372.14		0.6556695

				372.16		0.6556695

				372.19		0.6556695

				372.21		0.6556695

				372.23		0.6556695

				372.25		0.6556695

				372.27		0.6556695

				372.29		0.6556695

				372.31		0.6556695

				372.33		0.6556695

				372.36		0.6556695

				372.38		0.6556695

				372.4		0.6556695

				372.42		0.6556695

				372.44		0.6556695

				372.46		0.6556695

				372.48		0.6556695

				372.5		0.6556695

				372.53		0.6556695

				372.55		0.6556695

				372.57		0.6556695

				372.59		0.6556695

				372.61		0.6556695

				372.63		0.6556695

				372.65		0.6556695

				372.67		0.6556695

				372.7		0.6556695

				372.72		0.6556695

				372.74		0.6556695

				372.76		0.6556695

				372.78		0.6556695

				372.8		0.6556695

				372.82		0.6556695

				372.84		0.6556695

				372.87		0.6556695

				372.89		0.6556695

				372.91		0.6556695

				372.93		0.6556695

				372.95		0.6556695

				372.97		0.6556695

				372.99		0.6556695

				373.01		0.6556695

				373.04		0.6556695

				373.06		0.6504657

				373.08		0.6504657

				373.1		0.6504657

				373.12		0.6504657

				373.14		0.6504657

				373.16		0.6504657

				373.18		0.6504657

				373.2		0.6504657

				373.23		0.6504657

				373.25		0.6504657

				373.27		0.6504657

				373.29		0.6504657

				373.31		0.6504657

				373.33		0.6504657

				373.35		0.6504657

				373.37		0.6504657

				373.4		0.6504657

				373.42		0.6504657

				373.44		0.6504657

				373.46		0.6504657

				373.48		0.6504657

				373.5		0.6504657

				373.52		0.6504657

				373.54		0.6504657

				373.57		0.6504657

				373.59		0.6504657

				373.61		0.6504657

				373.63		0.6504657

				373.65		0.6504657

				373.67		0.6504657

				373.69		0.6504657

				373.71		0.6504657

				373.74		0.6504657

				373.76		0.6504657

				373.78		0.6504657

				373.8		0.6504657

				373.82		0.6504657

				373.84		0.6504657

				373.86		0.6504657

				373.88		0.6504657

				373.91		0.6504657

				373.93		0.6504657

				373.95		0.6504657

				373.97		0.6504657

				373.99		0.6504657

				374.01		0.6504657

				374.03		0.6504657

				374.05		0.6504657

				374.08		0.6504657

				374.1		0.6504657

				374.12		0.6504657

				374.14		0.6504657

				374.16		0.6504657

				374.18		0.6504657

				374.2		0.6504657

				374.22		0.6504657

				374.25		0.6504657

				374.27		0.6504657

				374.29		0.6504657

				374.31		0.645262

				374.33		0.6504657

				374.35		0.645262

				374.37		0.645262

				374.39		0.645262

				374.42		0.645262

				374.44		0.645262

				374.46		0.645262

				374.48		0.645262

				374.5		0.645262

				374.52		0.645262

				374.54		0.645262

				374.56		0.645262

				374.59		0.645262

				374.61		0.645262

				374.63		0.645262

				374.65		0.645262

				374.67		0.645262

				374.69		0.645262

				374.71		0.645262

				374.73		0.645262

				374.76		0.645262

				374.78		0.645262

				374.8		0.645262

				374.82		0.645262

				374.84		0.645262

				374.86		0.645262

				374.88		0.645262

				374.9		0.645262

				374.93		0.645262

				374.95		0.645262

				374.97		0.645262

				374.99		0.645262

				375.01		0.645262

				375.03		0.645262

				375.05		0.645262

				375.07		0.645262

				375.1		0.6504657

				375.12		0.645262

				375.14		0.645262

				375.16		0.645262

				375.18		0.6504657

				375.2		0.6504657

				375.22		0.6504657

				375.24		0.6504657

				375.27		0.6504657

				375.29		0.6504657

				375.31		0.6504657

				375.33		0.6504657

				375.35		0.6504657

				375.37		0.6504657

				375.39		0.6504657

				375.41		0.6504657

				375.44		0.6504657

				375.46		0.6504657

				375.48		0.6504657

				375.5		0.6504657

				375.52		0.6504657

				375.54		0.6504657

				375.56		0.6504657

				375.58		0.6504657

				375.61		0.6504657

				375.63		0.6504657

				375.65		0.6504657

				375.67		0.6504657

				375.69		0.6504657

				375.71		0.6504657

				375.73		0.6504657

				375.75		0.6504657

				375.78		0.6504657

				375.8		0.645262

				375.82		0.645262

				375.84		0.645262

				375.86		0.645262

				375.88		0.645262

				375.9		0.645262

				375.92		0.645262

				375.95		0.645262

				375.97		0.645262

				375.99		0.645262

				376.01		0.645262

				376.03		0.645262

				376.05		0.645262

				376.07		0.645262

				376.09		0.645262

				376.12		0.645262

				376.14		0.645262

				376.16		0.645262

				376.18		0.645262

				376.2		0.645262

				376.22		0.645262

				376.24		0.645262

				376.26		0.645262

				376.29		0.645262

				376.31		0.645262

				376.33		0.645262

				376.35		0.645262

				376.37		0.645262

				376.39		0.645262

				376.41		0.645262

				376.43		0.645262

				376.46		0.645262

				376.48		0.645262

				376.5		0.645262

				376.52		0.645262

				376.54		0.645262

				376.56		0.645262

				376.58		0.645262

				376.6		0.645262

				376.63		0.645262

				376.65		0.645262

				376.67		0.645262

				376.69		0.645262

				376.71		0.645262

				376.73		0.645262

				376.75		0.645262

				376.77		0.6400583

				376.8		0.6400583

				376.82		0.6400583

				376.84		0.6400583

				376.86		0.6400583

				376.88		0.6400583

				376.9		0.6400583

				376.92		0.6400583

				376.94		0.6400583

				376.97		0.6400583

				376.99		0.6400583

				377.01		0.6400583

				377.03		0.6400583

				377.05		0.6400583

				377.07		0.645262

				377.09		0.645262

				377.11		0.645262

				377.14		0.645262

				377.16		0.645262

				377.18		0.645262

				377.2		0.645262

				377.22		0.645262

				377.24		0.645262

				377.26		0.645262

				377.28		0.645262

				377.31		0.645262

				377.33		0.645262

				377.35		0.645262

				377.37		0.645262

				377.39		0.645262

				377.41		0.6400583

				377.43		0.6400583

				377.45		0.6400583

				377.48		0.6400583

				377.5		0.6400583

				377.52		0.6400583

				377.54		0.6400583

				377.56		0.6400583

				377.58		0.6400583

				377.6		0.6400583

				377.62		0.6400583

				377.65		0.6400583

				377.67		0.6400583

				377.69		0.6400583

				377.71		0.6400583

				377.73		0.6400583

				377.75		0.6400583

				377.77		0.6400583

				377.79		0.6400583

				377.81		0.6400583

				377.84		0.6400583

				377.86		0.6400583

				377.88		0.6400583

				377.9		0.6400583

				377.92		0.6400583

				377.94		0.6400583

				377.96		0.6400583

				377.98		0.6400583

				378.01		0.6400583

				378.03		0.6400583

				378.05		0.6400583

				378.07		0.6400583

				378.09		0.6400583

				378.11		0.6400583

				378.13		0.6348546

				378.15		0.6348546

				378.18		0.6348546

				378.2		0.6400583

				378.22		0.6348546

				378.24		0.6348546

				378.26		0.6348546

				378.28		0.6348546

				378.3		0.6348546

				378.32		0.6400583

				378.35		0.6400583

				378.37		0.6400583

				378.39		0.6400583

				378.41		0.6400583

				378.43		0.6400583

				378.45		0.6400583

				378.47		0.6348546

				378.49		0.6348546

				378.52		0.6348546

				378.54		0.6400583

				378.56		0.6348546

				378.58		0.6348546

				378.6		0.6348546

				378.62		0.6348546

				378.64		0.6348546

				378.66		0.6348546

				378.69		0.6348546

				378.71		0.6400583

				378.73		0.6348546

				378.75		0.6400583

				378.77		0.6400583

				378.79		0.6400583

				378.81		0.6348546

				378.83		0.6348546

				378.86		0.6348546

				378.88		0.6348546

				378.9		0.6348546

				378.92		0.6348546

				378.94		0.6348546

				378.96		0.6348546

				378.98		0.6348546

				379		0.6348546

				379.02		0.6348546

				379.05		0.6348546

				379.07		0.6348546

				379.09		0.6348546

				379.11		0.6348546

				379.13		0.6348546

				379.15		0.6348546

				379.17		0.6348546

				379.19		0.6348546

				379.22		0.6348546

				379.24		0.6296508

				379.26		0.6348546

				379.28		0.6296508

				379.3		0.6348546

				379.32		0.6296508

				379.34		0.6348546

				379.36		0.6348546

				379.39		0.6348546

				379.41		0.6348546

				379.43		0.6348546

				379.45		0.6348546

				379.47		0.6348546

				379.49		0.6296508

				379.51		0.6296508

				379.53		0.6348546

				379.56		0.6348546

				379.58		0.6296508

				379.6		0.6296508

				379.62		0.6296508

				379.64		0.6296508

				379.66		0.6296508

				379.68		0.6296508

				379.7		0.6296508

				379.73		0.6296508

				379.75		0.6296508

				379.77		0.6296508

				379.79		0.6296508

				379.81		0.6296508

				379.83		0.6296508

				379.85		0.6296508

				379.87		0.6296508

				379.9		0.6296508

				379.92		0.6296508

				379.94		0.6296508

				379.96		0.6296508

				379.98		0.6296508

				380		0.6296508

				380.02		0.6296508

				380.04		0.6296508

				380.07		0.6296508

				380.09		0.6296508

				380.11		0.6296508

				380.13		0.6296508

				380.15		0.6296508

				380.17		0.6296508

				380.19		0.6244471

				380.21		0.6244471

				380.24		0.6244471

				380.26		0.6244471

				380.28		0.6244471

				380.3		0.6244471

				380.32		0.6244471

				380.34		0.6244471

				380.36		0.6244471

				380.38		0.6244471

				380.41		0.6244471

				380.43		0.6244471

				380.45		0.6244471

				380.47		0.6244471

				380.49		0.6244471

				380.51		0.6244471

				380.53		0.6244471

				380.55		0.6244471

				380.58		0.6244471

				380.6		0.6244471

				380.62		0.6244471

				380.64		0.6244471

				380.66		0.6244471

				380.68		0.6244471

				380.7		0.6244471

				380.72		0.6244471

				380.75		0.6244471

				380.77		0.6244471

				380.79		0.6244471

				380.81		0.6244471

				380.83		0.6244471

				380.85		0.6244471

				380.87		0.6244471

				380.89		0.6244471

				380.91		0.6244471

				380.94		0.6192434

				380.96		0.6192434

				380.98		0.6244471

				381		0.6244471

				381.02		0.6244471

				381.04		0.6244471

				381.06		0.6192434

				381.08		0.6244471

				381.11		0.6192434

				381.13		0.6192434

				381.15		0.6192434

				381.17		0.6192434

				381.19		0.6192434

				381.21		0.6192434

				381.23		0.6192434

				381.25		0.6192434

				381.28		0.6192434

				381.3		0.6192434

				381.32		0.6192434

				381.34		0.6192434

				381.36		0.6192434

				381.38		0.6192434

				381.4		0.6192434

				381.42		0.6192434

				381.45		0.6192434

				381.47		0.6192434

				381.49		0.6192434

				381.51		0.6192434

				381.53		0.6192434

				381.55		0.6192434

				381.57		0.6192434

				381.59		0.6192434

				381.62		0.6192434

				381.64		0.6192434

				381.66		0.6192434

				381.68		0.6192434

				381.7		0.6192434

				381.72		0.6192434

				381.74		0.6192434

				381.76		0.6192434

				381.78		0.6192434

				381.81		0.6192434

				381.83		0.6192434

				381.85		0.6192434

				381.87		0.6192434

				381.89		0.6192434

				381.91		0.6192434

				381.93		0.6192434

				381.95		0.6192434

				381.98		0.6192434

				382		0.6192434

				382.02		0.6192434

				382.04		0.6192434

				382.06		0.6192434

				382.08		0.6192434

				382.1		0.6192434

				382.12		0.6192434

				382.15		0.6192434

				382.17		0.6192434

				382.19		0.6192434

				382.21		0.6192434

				382.23		0.6192434

				382.25		0.6192434

				382.27		0.6192434

				382.29		0.6192434

				382.32		0.6192434

				382.34		0.6192434

				382.36		0.6192434

				382.38		0.6192434

				382.4		0.6192434

				382.42		0.6192434

				382.44		0.6192434

				382.46		0.6192434

				382.48		0.6192434

				382.51		0.6192434

				382.53		0.6192434

				382.55		0.6192434

				382.57		0.6192434

				382.59		0.6192434

				382.61		0.6244471

				382.63		0.6192434

				382.65		0.6192434

				382.68		0.6192434

				382.7		0.6192434

				382.72		0.6192434

				382.74		0.6192434

				382.76		0.6192434

				382.78		0.6192434

				382.8		0.6192434

				382.82		0.6192434

				382.85		0.6192434

				382.87		0.6192434

				382.89		0.6192434

				382.91		0.6244471

				382.93		0.6244471

				382.95		0.6244471

				382.97		0.6244471

				382.99		0.6244471

				383.02		0.6244471

				383.04		0.6244471

				383.06		0.6244471

				383.08		0.6244471

				383.1		0.6244471

				383.12		0.6244471

				383.14		0.6296508

				383.16		0.6244471

				383.19		0.6244471

				383.21		0.6244471

				383.23		0.6244471

				383.25		0.6244471

				383.27		0.6296508

				383.29		0.6296508

				383.31		0.6296508

				383.33		0.6296508

				383.36		0.6296508

				383.38		0.6296508

				383.4		0.6296508

				383.42		0.6296508

				383.44		0.6296508

				383.46		0.6296508

				383.48		0.6296508

				383.5		0.6296508

				383.52		0.6296508

				383.55		0.6296508

				383.57		0.6296508

				383.59		0.6296508

				383.61		0.6296508

				383.63		0.6296508

				383.65		0.6296508

				383.67		0.6296508

				383.69		0.6296508

				383.72		0.6296508

				383.74		0.6296508

				383.76		0.6296508

				383.78		0.6296508

				383.8		0.6296508

				383.82		0.6296508

				383.84		0.6296508

				383.86		0.6296508

				383.89		0.6348546

				383.91		0.6348546

				383.93		0.6348546

				383.95		0.6348546

				383.97		0.6348546

				383.99		0.6348546

				384.01		0.6348546

				384.03		0.6348546

				384.06		0.6348546

				384.08		0.6348546

				384.1		0.6348546

				384.12		0.6348546

				384.14		0.6348546

				384.16		0.6348546

				384.18		0.6348546

				384.2		0.6348546

				384.23		0.6348546

				384.25		0.6348546

				384.27		0.6348546

				384.29		0.6348546

				384.31		0.6348546

				384.33		0.6348546

				384.35		0.6348546

				384.37		0.6400583

				384.4		0.6348546

				384.42		0.6400583

				384.44		0.6400583

				384.46		0.6348546

				384.48		0.6348546

				384.5		0.6348546

				384.52		0.6348546

				384.54		0.6348546

				384.56		0.6348546

				384.59		0.6400583

				384.61		0.6348546

				384.63		0.6348546

				384.65		0.6348546

				384.67		0.6400583

				384.69		0.6348546

				384.71		0.6348546

				384.73		0.6400583

				384.76		0.6400583

				384.78		0.6400583

				384.8		0.6400583

				384.82		0.6400583

				384.84		0.6400583

				384.86		0.6400583

				384.88		0.6400583

				384.9		0.6400583

				384.93		0.6400583

				384.95		0.6400583

				384.97		0.6400583

				384.99		0.6400583

				385.01		0.6400583

				385.03		0.6400583

				385.05		0.6400583

				385.07		0.6400583

				385.1		0.6400583

				385.12		0.6400583

				385.14		0.6400583

				385.16		0.6400583

				385.18		0.6400583

				385.2		0.6400583

				385.22		0.6400583

				385.24		0.6348546

				385.27		0.6400583

				385.29		0.6348546

				385.31		0.6400583

				385.33		0.6348546

				385.35		0.6348546

				385.37		0.6348546

				385.39		0.6348546

				385.41		0.6348546

				385.44		0.6348546

				385.46		0.6348546

				385.48		0.6348546

				385.5		0.6348546

				385.52		0.6400583

				385.54		0.6400583

				385.56		0.6400583

				385.58		0.6400583

				385.6		0.6400583

				385.63		0.6400583

				385.65		0.6400583

				385.67		0.6400583

				385.69		0.6400583

				385.71		0.6400583

				385.73		0.6400583

				385.75		0.6400583

				385.77		0.6400583

				385.8		0.6400583

				385.82		0.6400583

				385.84		0.6400583

				385.86		0.6400583

				385.88		0.6400583

				385.9		0.6400583

				385.92		0.6400583

				385.94		0.6400583

				385.97		0.6400583

				385.99		0.6400583

				386.01		0.6400583

				386.03		0.6400583

				386.05		0.6400583

				386.07		0.6400583

				386.09		0.6400583

				386.11		0.6400583

				386.14		0.6400583

				386.16		0.6400583

				386.18		0.6348546

				386.2		0.6400583

				386.22		0.6348546

				386.24		0.6348546

				386.26		0.6348546

				386.28		0.6348546

				386.31		0.6348546

				386.33		0.6348546

				386.35		0.6348546

				386.37		0.6348546

				386.39		0.6348546

				386.41		0.6348546

				386.43		0.6348546

				386.45		0.6348546

				386.47		0.6348546

				386.5		0.6348546

				386.52		0.6348546

				386.54		0.6348546

				386.56		0.6348546

				386.58		0.6348546

				386.6		0.6348546

				386.62		0.6348546

				386.64		0.6348546

				386.67		0.6348546

				386.69		0.6348546

				386.71		0.6348546

				386.73		0.6348546

				386.75		0.6348546

				386.77		0.6348546

				386.79		0.6348546

				386.81		0.6348546

				386.84		0.6348546

				386.86		0.6348546

				386.88		0.6348546

				386.9		0.6348546

				386.92		0.6348546

				386.94		0.6348546

				386.96		0.6348546

				386.98		0.6348546

				387.01		0.6348546

				387.03		0.6348546

				387.05		0.6348546

				387.07		0.6348546

				387.09		0.6348546

				387.11		0.6348546

				387.13		0.6348546

				387.15		0.6348546

				387.17		0.6348546

				387.2		0.6348546

				387.22		0.6348546

				387.24		0.6348546

				387.26		0.6296508

				387.28		0.6348546

				387.3		0.6348546

				387.32		0.6348546

				387.34		0.6348546

				387.37		0.6348546

				387.39		0.6348546

				387.41		0.6348546

				387.43		0.6348546

				387.45		0.6348546

				387.47		0.6348546

				387.49		0.6348546

				387.51		0.6348546

				387.53		0.6348546

				387.56		0.6348546

				387.58		0.6348546

				387.6		0.6348546

				387.62		0.6348546

				387.64		0.6348546

				387.66		0.6348546

				387.68		0.6296508

				387.7		0.6296508

				387.73		0.6296508

				387.75		0.6296508

				387.77		0.6296508

				387.79		0.6296508

				387.81		0.6296508

				387.83		0.6296508

				387.85		0.6296508

				387.87		0.6348546

				387.89		0.6348546

				387.92		0.6296508

				387.94		0.6296508

				387.96		0.6348546

				387.98		0.6296508

				388		0.6296508

				388.02		0.6296508

				388.04		0.6296508

				388.06		0.6296508

				388.09		0.6296508

				388.11		0.6296508

				388.13		0.6296508

				388.15		0.6296508

				388.17		0.6296508

				388.19		0.6296508

				388.21		0.6296508

				388.23		0.6296508

				388.25		0.6296508

				388.28		0.6296508

				388.3		0.6296508

				388.32		0.6296508

				388.34		0.6296508

				388.36		0.6296508

				388.38		0.6296508

				388.4		0.6296508

				388.42		0.6296508

				388.45		0.6296508

				388.47		0.6296508

				388.49		0.6296508

				388.51		0.6296508

				388.53		0.6296508

				388.55		0.6296508

				388.57		0.6296508

				388.59		0.6296508

				388.62		0.6296508

				388.64		0.6296508

				388.66		0.6296508

				388.68		0.6296508

				388.7		0.6296508

				388.72		0.6296508

				388.74		0.6296508

				388.76		0.6296508

				388.78		0.6296508

				388.81		0.6348546

				388.83		0.6296508

				388.85		0.6296508

				388.87		0.6348546

				388.89		0.6296508

				388.91		0.6296508

				388.93		0.6296508

				388.95		0.6296508

				388.98		0.6296508

				389		0.6296508

				389.02		0.6296508

				389.04		0.6296508

				389.06		0.6296508

				389.08		0.6296508

				389.1		0.6296508

				389.12		0.6296508

				389.14		0.6296508

				389.17		0.6296508

				389.19		0.6296508

				389.21		0.6296508

				389.23		0.6296508

				389.25		0.6296508

				389.27		0.6296508

				389.29		0.6296508

				389.31		0.6296508

				389.34		0.6296508

				389.36		0.6296508

				389.38		0.6296508

				389.4		0.6296508

				389.42		0.6296508

				389.44		0.6296508

				389.46		0.6296508

				389.48		0.6296508

				389.5		0.6296508

				389.53		0.6296508

				389.55		0.6296508

				389.57		0.6296508

				389.59		0.6296508

				389.61		0.6296508

				389.63		0.6296508

				389.65		0.6296508

				389.67		0.6296508

				389.7		0.6296508

				389.72		0.6296508

				389.74		0.6348546

				389.76		0.6348546

				389.78		0.6348546

				389.8		0.6348546

				389.82		0.6348546

				389.84		0.6348546

				389.86		0.6348546

				389.89		0.6348546

				389.91		0.6348546

				389.93		0.6296508

				389.95		0.6348546

				389.97		0.6348546

				389.99		0.6296508

				390.01		0.6348546

				390.03		0.6348546

				390.06		0.6348546

				390.08		0.6348546

				390.1		0.6348546

				390.12		0.6348546

				390.14		0.6348546

				390.16		0.6348546

				390.18		0.6348546

				390.2		0.6348546

				390.22		0.6348546

				390.25		0.6348546

				390.27		0.6348546

				390.29		0.6348546

				390.31		0.6348546

				390.33		0.6348546

				390.35		0.6348546

				390.37		0.6348546

				390.39		0.6348546

				390.41		0.6348546

				390.44		0.6348546

				390.46		0.6348546

				390.48		0.6348546

				390.5		0.6348546

				390.52		0.6348546

				390.54		0.6348546

				390.56		0.6348546

				390.58		0.6348546

				390.61		0.6348546

				390.63		0.6348546

				390.65		0.6348546

				390.67		0.6348546

				390.69		0.6348546

				390.71		0.6348546

				390.73		0.6348546

				390.75		0.6348546

				390.77		0.6348546

				390.8		0.6348546

				390.82		0.6348546

				390.84		0.6348546

				390.86		0.6348546

				390.88		0.6348546

				390.9		0.6348546

				390.92		0.6348546

				390.94		0.6348546

				390.96		0.6348546

				390.99		0.6348546

				391.01		0.6348546

				391.03		0.6348546

				391.05		0.6348546

				391.07		0.6348546

				391.09		0.6348546

				391.11		0.6348546

				391.13		0.6348546

				391.16		0.6348546

				391.18		0.6348546

				391.2		0.6348546

				391.22		0.6348546

				391.24		0.6348546

				391.26		0.6348546

				391.28		0.6348546

				391.3		0.6348546

				391.32		0.6348546

				391.35		0.6348546

				391.37		0.6348546

				391.39		0.6348546

				391.41		0.6348546

				391.43		0.6348546

				391.45		0.6348546

				391.47		0.6348546

				391.49		0.6348546

				391.52		0.6348546

				391.54		0.6296508

				391.56		0.6348546

				391.58		0.6296508

				391.6		0.6348546

				391.62		0.6296508

				391.64		0.6348546

				391.66		0.6348546

				391.68		0.6348546

				391.71		0.6348546

				391.73		0.6296508

		Results:

		Onset		X1		188.64		°C

				Y1		95.01		%

				X2		252.14		°C

				Y2		7.505		%

				Onset X		231.91		°C

				Onset Y		83.751		%
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RT-54-0.2 GnP.xlsx
Sheet1

		Method Filename:		C:\Program Files (x86)\PerkinElmer\Pyris\data\Anas\21052024\RT54-GNP 0.2.t6d

		Sample ID:		RT54-GNP 0.2

		Step:		1

		Data		Sample Temperature (°C)		Weight % (%)

				30.07		100.0194

				30.07		100.0155

				30.07		100.0155

				30.07		100.0194

				30.07		100.0194

				30.07		100.0194

				30.07		100.0194

				30.07		100.0194

				30.07		100.0194

				30.07		100.0194

				30.07		100.0194

				30.07		100.0194

				30.07		100.0194

				30.07		100.0194

				30.07		100.0233

				30.07		100.0233

				30.07		100.0233

				30.07		100.0233

				30.07		100.0233

				30.07		100.0233

				30.07		100.0233

				30.07		100.0233

				30.07		100.0233

				30.07		100.0233

				30.07		100.0233

				30.07		100.0233

				30.07		100.0233

				30.07		100.0233

				30.07		100.0233

				30.07		100.0233

				30.07		100.0233

				30.07		100.0233

				30.07		100.0233

				30.07		100.0233

				30.07		100.0233

				30.07		100.0233

				30.07		100.0233

				30.07		100.0233

				30.07		100.0272

				30.07		100.0272

				30.07		100.0272

				30.07		100.0272

				30.07		100.0272

				30.06		100.0272

				30.06		100.0272

				30.06		100.0272

				30.06		100.0272

				30.06		100.0272

				30.06		100.0272

				30.06		100.0272

				30.06		100.0272

				30.06		100.0272

				30.06		100.0272

				30.06		100.0272

				30.06		100.0272

				30.06		100.0272

				30.06		100.0272

				30.06		100.0272

				30.06		100.031

				30.06		100.031

				30.06		100.031

				30.06		100.031

				30.06		100.031

				30.06		100.031

				30.06		100.031

				30.06		100.031

				30.06		100.031

				30.06		100.0349

				30.06		100.0349

				30.06		100.0349

				30.06		100.0349

				30.06		100.0349

				30.06		100.0349

				30.06		100.0349

				30.06		100.0349

				30.06		100.0349

				30.06		100.0349

				30.06		100.0349

				30.06		100.0388

				30.06		100.0388

				30.06		100.0388

				30.06		100.0388

				30.06		100.0388

				30.06		100.0388

				30.06		100.0388

				30.06		100.0388

				30.07		100.0388

				30.07		100.0388

				30.07		100.0388

				30.07		100.0388

				30.07		100.0427

				30.07		100.0427

				30.07		100.0427

				30.07		100.0427

				30.07		100.0427

				30.07		100.0427

				30.07		100.0466

				30.07		100.0466

				30.07		100.0466

				30.07		100.0466

				30.07		100.0466

				30.07		100.0466

				30.07		100.0466

				30.07		100.0466

				30.07		100.0466

				30.07		100.0504

				30.07		100.0504

				30.07		100.0504

				30.07		100.0504

				30.07		100.0504

				30.07		100.0504

				30.07		100.0543

				30.07		100.0543

				30.07		100.0543

				30.08		100.0543

				30.08		100.0543

				30.08		100.0543

				30.08		100.0582

				30.08		100.0582

				30.08		100.0582

				30.08		100.0582

				30.08		100.0582

				30.08		100.0582

				30.08		100.0582

				30.08		100.0621

				30.08		100.0621

				30.09		100.0621

				30.09		100.0621

				30.09		100.0621

				30.09		100.0621

				30.09		100.0621

				30.09		100.0621

				30.09		100.0621

				30.09		100.0621

				30.1		100.0621

				30.1		100.0621

				30.1		100.0621

				30.1		100.066

				30.1		100.066

				30.1		100.066

				30.1		100.066

				30.11		100.066

				30.11		100.066

				30.11		100.066

				30.11		100.066

				30.11		100.066

				30.12		100.0698

				30.12		100.0698

				30.12		100.0698

				30.12		100.0698

				30.12		100.0698

				30.13		100.0698

				30.13		100.0698

				30.13		100.0698

				30.13		100.0737

				30.13		100.0737

				30.14		100.0737

				30.14		100.0737

				30.14		100.0737

				30.14		100.0737

				30.15		100.0737

				30.15		100.0737

				30.15		100.0737

				30.15		100.0737

				30.16		100.0737

				30.16		100.0737

				30.16		100.0737

				30.16		100.0737

				30.17		100.0737

				30.17		100.0737

				30.17		100.0737

				30.18		100.0776

				30.18		100.0776

				30.18		100.0776

				30.19		100.0776

				30.19		100.0776

				30.19		100.0776

				30.19		100.0776

				30.2		100.0776

				30.2		100.0776

				30.2		100.0776

				30.21		100.0776

				30.21		100.0776

				30.22		100.0815

				30.22		100.0815

				30.22		100.0815

				30.23		100.0815

				30.23		100.0815

				30.23		100.0815

				30.24		100.0815

				30.24		100.0815

				30.24		100.0815

				30.25		100.0815

				30.25		100.0815

				30.26		100.0815

				30.26		100.0815

				30.26		100.0815

				30.27		100.0854

				30.27		100.0854

				30.28		100.0854

				30.28		100.0854

				30.28		100.0854

				30.29		100.0854

				30.29		100.0854

				30.3		100.0854

				30.3		100.0854

				30.31		100.0854

				30.31		100.0892

				30.31		100.0892

				30.32		100.0892

				30.32		100.0892

				30.33		100.0892

				30.33		100.0892

				30.34		100.0892

				30.34		100.0892

				30.35		100.0892

				30.35		100.0931

				30.36		100.0931

				30.36		100.0931

				30.37		100.0931

				30.37		100.0931

				30.38		100.0931

				30.38		100.0931

				30.39		100.0931

				30.39		100.0931

				30.4		100.0931

				30.4		100.097

				30.41		100.097

				30.41		100.097

				30.42		100.097

				30.42		100.097

				30.43		100.097

				30.43		100.097

				30.44		100.097

				30.44		100.097

				30.45		100.097

				30.46		100.1009

				30.46		100.097

				30.47		100.1009

				30.47		100.1009

				30.48		100.1009

				30.48		100.1009

				30.49		100.1009

				30.5		100.1009

				30.5		100.1009

				30.51		100.1009

				30.51		100.1009

				30.52		100.1009

				30.52		100.1009

				30.53		100.1009

				30.54		100.1009

				30.54		100.1048

				30.55		100.1009

				30.55		100.1009

				30.56		100.1048

				30.57		100.1048

				30.57		100.1048

				30.58		100.1048

				30.59		100.1048

				30.59		100.1048

				30.6		100.1048

				30.6		100.1048

				30.61		100.1048

				30.62		100.1086

				30.62		100.1048

				30.63		100.1086

				30.64		100.1086

				30.64		100.1086

				30.65		100.1086

				30.66		100.1086

				30.66		100.1086

				30.67		100.1086

				30.68		100.1086

				30.68		100.1086

				30.69		100.1086

				30.7		100.1086

				30.7		100.1125

				30.71		100.1125

				30.72		100.1086

				30.72		100.1125

				30.73		100.1125

				30.74		100.1125

				30.75		100.1125

				30.75		100.1125

				30.76		100.1125

				30.77		100.1125

				30.77		100.1125

				30.78		100.1125

				30.79		100.1125

				30.8		100.1125

				30.8		100.1125

				30.81		100.1164

				30.82		100.1125

				30.82		100.1125

				30.83		100.1164

				30.84		100.1164

				30.85		100.1164

				30.85		100.1164

				30.86		100.1164

				30.87		100.1164

				30.88		100.1164

				30.88		100.1164

				30.89		100.1164

				30.9		100.1164

				30.91		100.1164

				30.91		100.1164

				30.92		100.1164

				30.93		100.1164

				30.94		100.1164

				30.94		100.1164

				30.95		100.1164

				30.96		100.1164

				30.97		100.1164

				30.98		100.1164

				30.98		100.1164

				30.99		100.1164

				31		100.1164

				31.01		100.1164

				31.02		100.1164

				31.02		100.1203

				31.03		100.1164

				31.04		100.1203

				31.05		100.1203

				31.06		100.1203

				31.06		100.1203

				31.07		100.1203

				31.08		100.1203

				31.09		100.1203

				31.1		100.1203

				31.1		100.1203

				31.11		100.1203

				31.12		100.1203

				31.13		100.1203

				31.14		100.1203

				31.15		100.1203

				31.15		100.1203

				31.16		100.1242

				31.17		100.1242

				31.18		100.1242

				31.19		100.1242

				31.2		100.1242

				31.21		100.1242

				31.21		100.1242

				31.22		100.1242

				31.23		100.1242

				31.24		100.1242

				31.25		100.128

				31.26		100.1242

				31.27		100.128

				31.27		100.128

				31.28		100.128

				31.29		100.128

				31.3		100.128

				31.31		100.128

				31.32		100.128

				31.33		100.1319

				31.34		100.1319

				31.35		100.1319

				31.35		100.1319

				31.36		100.1319

				31.37		100.1319

				31.38		100.1319

				31.39		100.1319

				31.4		100.1319

				31.41		100.1319

				31.42		100.1319

				31.43		100.1319

				31.44		100.1358

				31.44		100.1358

				31.45		100.1358

				31.46		100.1358

				31.47		100.1358

				31.48		100.1358

				31.49		100.1358

				31.5		100.1358

				31.51		100.1358

				31.52		100.1358

				31.53		100.1397

				31.54		100.1358

				31.55		100.1397

				31.56		100.1397

				31.57		100.1397

				31.57		100.1397

				31.58		100.1397

				31.59		100.1397

				31.6		100.1397

				31.61		100.1397

				31.62		100.1397

				31.63		100.1397

				31.64		100.1397

				31.65		100.1397

				31.66		100.1397

				31.67		100.1397

				31.68		100.1436

				31.69		100.1436

				31.7		100.1436

				31.71		100.1436

				31.72		100.1436

				31.73		100.1436

				31.74		100.1436

				31.75		100.1436

				31.76		100.1436

				31.77		100.1436

				31.78		100.1436

				31.79		100.1436

				31.8		100.1436

				31.81		100.1436

				31.82		100.1474

				31.83		100.1474

				31.84		100.1474

				31.85		100.1474

				31.86		100.1474

				31.87		100.1474

				31.88		100.1474

				31.89		100.1474

				31.9		100.1474

				31.91		100.1474

				31.92		100.1474

				31.93		100.1474

				31.94		100.1474

				31.95		100.1474

				31.96		100.1474

				31.97		100.1474

				31.98		100.1474

				31.99		100.1474

				32		100.1474

				32.01		100.1474

				32.02		100.1474

				32.03		100.1474

				32.04		100.1474

				32.05		100.1474

				32.06		100.1474

				32.07		100.1474

				32.08		100.1474

				32.09		100.1474

				32.11		100.1474

				32.12		100.1474

				32.13		100.1474

				32.14		100.1474

				32.15		100.1474

				32.16		100.1474

				32.17		100.1474

				32.18		100.1474

				32.19		100.1474

				32.2		100.1474

				32.21		100.1474

				32.22		100.1474

				32.23		100.1474

				32.24		100.1474

				32.26		100.1474

				32.27		100.1474

				32.28		100.1474

				32.29		100.1474

				32.3		100.1474

				32.31		100.1474

				32.32		100.1513

				32.33		100.1513

				32.34		100.1513

				32.35		100.1513

				32.36		100.1513

				32.38		100.1513

				32.39		100.1513

				32.4		100.1513

				32.41		100.1513

				32.42		100.1513

				32.43		100.1513

				32.44		100.1513

				32.45		100.1513

				32.46		100.1513

				32.48		100.1513

				32.49		100.1513

				32.5		100.1513

				32.51		100.1513

				32.52		100.1513

				32.53		100.1513

				32.54		100.1513

				32.55		100.1513

				32.57		100.1513

				32.58		100.1513

				32.59		100.1513

				32.6		100.1552

				32.61		100.1552

				32.62		100.1552

				32.63		100.1552

				32.65		100.1552

				32.66		100.1552

				32.67		100.1552

				32.68		100.1552

				32.69		100.1552

				32.7		100.1552

				32.71		100.1552

				32.73		100.1552

				32.74		100.1552

				32.75		100.1552

				32.76		100.1552

				32.77		100.1552

				32.78		100.1552

				32.8		100.1591

				32.81		100.1552

				32.82		100.1552

				32.83		100.1591

				32.84		100.1591

				32.86		100.1591

				32.87		100.1591

				32.88		100.1591

				32.89		100.1591

				32.9		100.1591

				32.91		100.1591

				32.93		100.163

				32.94		100.163

				32.95		100.163

				32.96		100.163

				32.97		100.163

				32.99		100.163

				33		100.163

				33.01		100.163

				33.02		100.163

				33.03		100.163

				33.05		100.1668

				33.06		100.1668

				33.07		100.1668

				33.08		100.1668

				33.1		100.1668

				33.11		100.1668

				33.12		100.1707

				33.13		100.1707

				33.14		100.1707

				33.16		100.1707

				33.17		100.1707

				33.18		100.1707

				33.19		100.1707

				33.21		100.1707

				33.22		100.1707

				33.23		100.1707

				33.24		100.1707

				33.25		100.1707

				33.27		100.1707

				33.28		100.1707

				33.29		100.1707

				33.3		100.1707

				33.32		100.1746

				33.33		100.1746

				33.34		100.1746

				33.35		100.1746

				33.37		100.1746

				33.38		100.1746

				33.39		100.1746

				33.4		100.1746

				33.42		100.1785

				33.43		100.1785

				33.44		100.1785

				33.46		100.1785

				33.47		100.1785

				33.48		100.1785

				33.49		100.1785

				33.51		100.1785

				33.52		100.1785

				33.53		100.1785

				33.54		100.1785

				33.56		100.1785

				33.57		100.1785

				33.58		100.1824

				33.6		100.1824

				33.61		100.1824

				33.62		100.1824

				33.63		100.1824

				33.65		100.1824

				33.66		100.1824

				33.67		100.1824

				33.69		100.1824

				33.7		100.1824

				33.71		100.1824

				33.72		100.1824

				33.74		100.1862

				33.75		100.1862

				33.76		100.1862

				33.78		100.1862

				33.79		100.1862

				33.8		100.1862

				33.82		100.1862

				33.83		100.1862

				33.84		100.1862

				33.86		100.1862

				33.87		100.1862

				33.88		100.1862

				33.9		100.1862

				33.91		100.1862

				33.92		100.1862

				33.93		100.1862

				33.95		100.1862

				33.96		100.1862

				33.97		100.1862

				33.99		100.1901

				34		100.1901

				34.01		100.1862

				34.03		100.1901

				34.04		100.1901

				34.05		100.1901

				34.07		100.1901

				34.08		100.1901

				34.09		100.1901

				34.11		100.1901

				34.12		100.1901

				34.13		100.1901

				34.15		100.1901

				34.16		100.1901

				34.18		100.1862

				34.19		100.1862

				34.2		100.1862

				34.22		100.1901

				34.23		100.1901

				34.24		100.1901

				34.26		100.1901

				34.27		100.1901

				34.28		100.1901

				34.3		100.1901

				34.31		100.1901

				34.32		100.1901

				34.34		100.1901

				34.35		100.1901

				34.37		100.1901

				34.38		100.1901

				34.39		100.1901

				34.41		100.1862

				34.42		100.1862

				34.43		100.1862

				34.45		100.1901

				34.46		100.1901

				34.48		100.1862

				34.49		100.1901

				34.5		100.1862

				34.52		100.1862

				34.53		100.1862

				34.55		100.1901

				34.56		100.1901

				34.57		100.1901

				34.59		100.1901

				34.6		100.1901

				34.61		100.1901

				34.63		100.1901

				34.64		100.1901

				34.66		100.1901

				34.67		100.1901

				34.69		100.1901

				34.7		100.1901

				34.71		100.1901

				34.73		100.1901

				34.74		100.1901

				34.76		100.1901

				34.77		100.1901

				34.78		100.1901

				34.8		100.1901

				34.81		100.1901

				34.83		100.1901

				34.84		100.1901

				34.85		100.1901

				34.87		100.1901

				34.88		100.1901

				34.9		100.1901

				34.91		100.1901

				34.93		100.1901

				34.94		100.1901

				34.95		100.1901

				34.97		100.1901

				34.98		100.1901

				35		100.1901

				35.01		100.194

				35.03		100.194

				35.04		100.194

				35.05		100.194

				35.07		100.194

				35.08		100.194

				35.1		100.194

				35.11		100.194

				35.13		100.194

				35.14		100.194

				35.16		100.194

				35.17		100.194

				35.18		100.194

				35.2		100.194

				35.21		100.194

				35.23		100.194

				35.24		100.194

				35.26		100.194

				35.27		100.194

				35.29		100.194

				35.3		100.194

				35.32		100.194

				35.33		100.194

				35.35		100.1979

				35.36		100.194

				35.37		100.1979

				35.39		100.1979

				35.4		100.1979

				35.42		100.1979

				35.43		100.1979

				35.45		100.1979

				35.46		100.1979

				35.48		100.1979

				35.49		100.1979

				35.51		100.1979

				35.52		100.1979

				35.54		100.1979

				35.55		100.1979

				35.57		100.1979

				35.58		100.1979

				35.6		100.1979

				35.61		100.1979

				35.63		100.1979

				35.64		100.1979

				35.66		100.1979

				35.67		100.1979

				35.69		100.2018

				35.7		100.1979

				35.72		100.2018

				35.73		100.2018

				35.75		100.2018

				35.76		100.2018

				35.78		100.2018

				35.79		100.2018

				35.81		100.2018

				35.82		100.2018

				35.84		100.2018

				35.85		100.2018

				35.87		100.2018

				35.88		100.2018

				35.9		100.2018

				35.91		100.2056

				35.93		100.2056

				35.94		100.2056

				35.96		100.2056

				35.97		100.2056

				35.99		100.2056

				36		100.2056

				36.02		100.2056

				36.03		100.2056

				36.05		100.2056

				36.06		100.2056

				36.08		100.2095

				36.09		100.2095

				36.11		100.2095

				36.12		100.2095

				36.14		100.2095

				36.15		100.2095

				36.17		100.2095

				36.18		100.2095

				36.2		100.2095

				36.21		100.2095

				36.23		100.2095

				36.25		100.2095

				36.26		100.2095

				36.28		100.2095

				36.29		100.2095

				36.31		100.2095

				36.32		100.2095

				36.34		100.2095

				36.35		100.2134

				36.37		100.2095

				36.38		100.2134

				36.4		100.2134

				36.42		100.2095

				36.43		100.2134

				36.45		100.2134

				36.46		100.2134

				36.48		100.2095

				36.49		100.2134

				36.51		100.2134

				36.52		100.2134

				36.54		100.2134

				36.55		100.2134

				36.57		100.2134

				36.59		100.2134

				36.6		100.2134

				36.62		100.2134

				36.63		100.2134

				36.65		100.2134

				36.66		100.2134

				36.68		100.2173

				36.7		100.2134

				36.71		100.2134

				36.73		100.2134

				36.74		100.2134

				36.76		100.2134

				36.77		100.2134

				36.79		100.2134

				36.81		100.2134

				36.82		100.2173

				36.84		100.2134

				36.85		100.2134

				36.87		100.2173

				36.88		100.2173

				36.9		100.2173

				36.92		100.2173

				36.93		100.2173

				36.95		100.2173

				36.96		100.2173

				36.98		100.2173

				37		100.2173

				37.01		100.2173

				37.03		100.2212

				37.04		100.2212

				37.06		100.2212

				37.07		100.2212

				37.09		100.2212

				37.11		100.2212

				37.12		100.2212

				37.14		100.2212

				37.15		100.2212

				37.17		100.2212

				37.19		100.2212

				37.2		100.2212

				37.22		100.2212

				37.23		100.2212

				37.25		100.2212

				37.27		100.2212

				37.28		100.2212

				37.3		100.225

				37.31		100.2212

				37.33		100.2212

				37.35		100.2212

				37.36		100.225

				37.38		100.225

				37.39		100.225

				37.41		100.225

				37.43		100.225

				37.44		100.225

				37.46		100.225

				37.48		100.225

				37.49		100.225

				37.51		100.225

				37.52		100.225

				37.54		100.225

				37.56		100.225

				37.57		100.225

				37.59		100.225

				37.61		100.225

				37.62		100.225

				37.64		100.225

				37.65		100.225

				37.67		100.225

				37.69		100.225

				37.7		100.225

				37.72		100.225

				37.74		100.225

				37.75		100.225

				37.77		100.2289

				37.78		100.225

				37.8		100.2289

				37.82		100.225

				37.83		100.225

				37.85		100.225

				37.87		100.2289

				37.88		100.2289

				37.9		100.225

				37.92		100.2289

				37.93		100.2289

				37.95		100.2289

				37.97		100.2289

				37.98		100.2289

				38		100.2289

				38.01		100.2289

				38.03		100.2289

				38.05		100.2289

				38.06		100.2289

				38.08		100.2289

				38.1		100.2289

				38.11		100.2289

				38.13		100.2289

				38.15		100.2289

				38.16		100.2289

				38.18		100.2289

				38.2		100.2289

				38.21		100.2289

				38.23		100.2289

				38.25		100.2289

				38.26		100.2289

				38.28		100.2289

				38.3		100.2289

				38.31		100.2289

				38.33		100.2289

				38.35		100.2289

				38.36		100.2328

				38.38		100.2328

				38.4		100.2328

				38.41		100.2328

				38.43		100.2328

				38.45		100.2328

				38.46		100.2328

				38.48		100.2328

				38.5		100.2328

				38.51		100.2328

				38.53		100.2328

				38.55		100.2328

				38.56		100.2328

				38.58		100.2328

				38.6		100.2328

				38.61		100.2328

				38.63		100.2328

				38.65		100.2328

				38.66		100.2328

				38.68		100.2328

				38.7		100.2328

				38.71		100.2328

				38.73		100.2328

				38.75		100.2367

				38.76		100.2328

				38.78		100.2367

				38.8		100.2367

				38.82		100.2367

				38.83		100.2367

				38.85		100.2367

				38.87		100.2367

				38.88		100.2367

				38.9		100.2367

				38.92		100.2367

				38.93		100.2367

				38.95		100.2406

				38.97		100.2406

				38.98		100.2406

				39		100.2406

				39.02		100.2367

				39.04		100.2406

				39.05		100.2406

				39.07		100.2406

				39.09		100.2406

				39.1		100.2406

				39.12		100.2406

				39.14		100.2406

				39.16		100.2406

				39.17		100.2406

				39.19		100.2406

				39.21		100.2406

				39.22		100.2406

				39.24		100.2406

				39.26		100.2406

				39.27		100.2406

				39.29		100.2444

				39.31		100.2444

				39.33		100.2444

				39.34		100.2444

				39.36		100.2444

				39.38		100.2444

				39.39		100.2444

				39.41		100.2444

				39.43		100.2444

				39.45		100.2444

				39.46		100.2444

				39.48		100.2444

				39.5		100.2444

				39.51		100.2444

				39.53		100.2444

				39.55		100.2444

				39.57		100.2444

				39.58		100.2444

				39.6		100.2444

				39.62		100.2444

				39.64		100.2483

				39.65		100.2483

				39.67		100.2483

				39.69		100.2483

				39.7		100.2483

				39.72		100.2483

				39.74		100.2483

				39.76		100.2444

				39.77		100.2483

				39.79		100.2483

				39.81		100.2483

				39.83		100.2483

				39.84		100.2483

				39.86		100.2483

				39.88		100.2483

				39.9		100.2483

				39.91		100.2483

				39.93		100.2483

				39.95		100.2483

				39.96		100.2483

				39.98		100.2483

				40		100.2483

				40.02		100.2483

				40.03		100.2483

				40.05		100.2483

				40.07		100.2483

				40.09		100.2483

				40.1		100.2483

				40.12		100.2483

				40.14		100.2483

				40.16		100.2483

				40.17		100.2522

				40.19		100.2522

				40.21		100.2522

				40.23		100.2522

				40.24		100.2522

				40.26		100.2522

				40.28		100.2522

				40.3		100.2522

				40.31		100.2522

				40.33		100.2522

				40.35		100.2522

				40.37		100.2522

				40.39		100.2522

				40.4		100.2522

				40.42		100.2522

				40.44		100.2522

				40.46		100.2522

				40.47		100.2522

				40.49		100.2522

				40.51		100.2522

				40.53		100.2522

				40.54		100.2522

				40.56		100.2522

				40.58		100.2522

				40.6		100.2522

				40.61		100.2522

				40.63		100.2522

				40.65		100.2522

				40.67		100.2522

				40.68		100.2522

				40.7		100.2522

				40.72		100.2522

				40.74		100.2522

				40.76		100.2522

				40.77		100.2522

				40.79		100.2522

				40.81		100.2522

				40.83		100.2522

				40.84		100.2522

				40.86		100.2522

				40.88		100.2522

				40.9		100.2561

				40.92		100.2561

				40.93		100.2522

				40.95		100.2522

				40.97		100.2522

				40.99		100.2522

				41		100.2522

				41.02		100.2522

				41.04		100.2522

				41.06		100.2522

				41.08		100.2522

				41.09		100.2522

				41.11		100.2522

				41.13		100.2522

				41.15		100.2522

				41.16		100.2561

				41.18		100.2522

				41.2		100.2561

				41.22		100.2561

				41.24		100.2561

				41.25		100.2561

				41.27		100.2561

				41.29		100.2561

				41.31		100.2561

				41.33		100.2561

				41.34		100.2561

				41.36		100.2561

				41.38		100.2561

				41.4		100.2561

				41.42		100.2561

				41.43		100.2561

				41.45		100.2561

				41.47		100.2561

				41.49		100.26

				41.51		100.2561

				41.52		100.2561

				41.54		100.2561

				41.56		100.26

				41.58		100.2561

				41.6		100.26

				41.61		100.26

				41.63		100.26

				41.65		100.26

				41.67		100.26

				41.69		100.26

				41.7		100.26

				41.72		100.26

				41.74		100.26

				41.76		100.26

				41.78		100.26

				41.79		100.26

				41.81		100.26

				41.83		100.26

				41.85		100.26

				41.87		100.26

				41.88		100.26

				41.9		100.26

				41.92		100.26

				41.94		100.26

				41.96		100.26

				41.97		100.26

				41.99		100.26

				42.01		100.26

				42.03		100.26

				42.05		100.26

				42.07		100.26

				42.08		100.26

				42.1		100.26

				42.12		100.26

				42.14		100.26

				42.16		100.26

				42.17		100.2638

				42.19		100.26

				42.21		100.26

				42.23		100.26

				42.25		100.26

				42.27		100.26

				42.28		100.26

				42.3		100.26

				42.32		100.26

				42.34		100.26

				42.36		100.26

				42.37		100.26

				42.39		100.26

				42.41		100.2638

				42.43		100.2638

				42.45		100.2638

				42.47		100.2638

				42.48		100.2638

				42.5		100.2638

				42.52		100.2638

				42.54		100.2638

				42.56		100.2638

				42.58		100.2638

				42.59		100.2638

				42.61		100.2638

				42.63		100.2638

				42.65		100.2638

				42.67		100.2638

				42.69		100.2638

				42.7		100.2638

				42.72		100.2638

				42.74		100.2638

				42.76		100.2638

				42.78		100.2638

				42.8		100.2638

				42.82		100.2638

				42.83		100.2638

				42.85		100.2638

				42.87		100.2638

				42.89		100.2638

				42.91		100.2638

				42.93		100.2638

				42.94		100.2638

				42.96		100.2638

				42.98		100.2638

				43		100.2638

				43.02		100.2638

				43.04		100.2638

				43.05		100.2638

				43.07		100.2638

				43.09		100.2638

				43.11		100.2638

				43.13		100.2638

				43.15		100.2638

				43.17		100.2638

				43.18		100.2638

				43.2		100.2638

				43.22		100.2638

				43.24		100.2638

				43.26		100.2638

				43.28		100.2638

				43.3		100.2638

				43.31		100.2638

				43.33		100.2638

				43.35		100.2638

				43.37		100.2638

				43.39		100.2638

				43.41		100.2638

				43.42		100.2677

				43.44		100.2638

				43.46		100.2677

				43.48		100.2677

				43.5		100.2677

				43.52		100.2638

				43.54		100.2677

				43.55		100.2677

				43.57		100.2638

				43.59		100.2677

				43.61		100.2677

				43.63		100.2677

				43.65		100.2677

				43.67		100.2677

				43.69		100.2677

				43.7		100.2677

				43.72		100.2677

				43.74		100.2677

				43.76		100.2677

				43.78		100.2677

				43.8		100.2677

				43.82		100.2677

				43.83		100.2677

				43.85		100.2677

				43.87		100.2677

				43.89		100.2677

				43.91		100.2677

				43.93		100.2677

				43.95		100.2677

				43.97		100.2677

				43.98		100.2677

				44		100.2677

				44.02		100.2677

				44.04		100.2677

				44.06		100.2677

				44.08		100.2677

				44.1		100.2677

				44.12		100.2677

				44.13		100.2677

				44.15		100.2677

				44.17		100.2677

				44.19		100.2677

				44.21		100.2677

				44.23		100.2716

				44.25		100.2716

				44.27		100.2716

				44.28		100.2716

				44.3		100.2716

				44.32		100.2716

				44.34		100.2716

				44.36		100.2716

				44.38		100.2716

				44.4		100.2716

				44.42		100.2716

				44.43		100.2716

				44.45		100.2716

				44.47		100.2716

				44.49		100.2716

				44.51		100.2716

				44.53		100.2716

				44.55		100.2755

				44.57		100.2755

				44.58		100.2755

				44.6		100.2755

				44.62		100.2755

				44.64		100.2755

				44.66		100.2755

				44.68		100.2755

				44.7		100.2755

				44.72		100.2755

				44.74		100.2755

				44.75		100.2755

				44.77		100.2755

				44.79		100.2755

				44.81		100.2794

				44.83		100.2794

				44.85		100.2755

				44.87		100.2755

				44.89		100.2794

				44.91		100.2755

				44.93		100.2755

				44.94		100.2794

				44.96		100.2755

				44.98		100.2794

				45		100.2794

				45.02		100.2794

				45.04		100.2794

				45.06		100.2794

				45.08		100.2794

				45.1		100.2794

				45.11		100.2755

				45.13		100.2755

				45.15		100.2794

				45.17		100.2794

				45.19		100.2794

				45.21		100.2794

				45.23		100.2794

				45.25		100.2794

				45.27		100.2794

				45.29		100.2794

				45.3		100.2794

				45.32		100.2755

				45.34		100.2794

				45.36		100.2794

				45.38		100.2794

				45.4		100.2794

				45.42		100.2794

				45.44		100.2794

				45.46		100.2794

				45.48		100.2794

				45.5		100.2794

				45.51		100.2794

				45.53		100.2794

				45.55		100.2794

				45.57		100.2794

				45.59		100.2794

				45.61		100.2794

				45.63		100.2794

				45.65		100.2794

				45.67		100.2794

				45.69		100.2794

				45.71		100.2794

				45.72		100.2794

				45.74		100.2794

				45.76		100.2794

				45.78		100.2794

				45.8		100.2794

				45.82		100.2794

				45.84		100.2794

				45.86		100.2794

				45.88		100.2794

				45.9		100.2794

				45.92		100.2794

				45.93		100.2794

				45.95		100.2832

				45.97		100.2794

				45.99		100.2832

				46.01		100.2832

				46.03		100.2832

				46.05		100.2832

				46.07		100.2832

				46.09		100.2832

				46.11		100.2832

				46.13		100.2832

				46.15		100.2832

				46.17		100.2794

				46.18		100.2832

				46.2		100.2832

				46.22		100.2794

				46.24		100.2832

				46.26		100.2794

				46.28		100.2794

				46.3		100.2794

				46.32		100.2794

				46.34		100.2794

				46.36		100.2832

				46.38		100.2832

				46.4		100.2794

				46.41		100.2794

				46.43		100.2794

				46.45		100.2794

				46.47		100.2832

				46.49		100.2794

				46.51		100.2832

				46.53		100.2832

				46.55		100.2832

				46.57		100.2832

				46.59		100.2832

				46.61		100.2832

				46.63		100.2832

				46.65		100.2832

				46.67		100.2832

				46.68		100.2832

				46.7		100.2794

				46.72		100.2832

				46.74		100.2832

				46.76		100.2832

				46.78		100.2832

				46.8		100.2832

				46.82		100.2832

				46.84		100.2832

				46.86		100.2832

				46.88		100.2832

				46.9		100.2832

				46.92		100.2832

				46.94		100.2832

				46.96		100.2832

				46.97		100.2832

				46.99		100.2832

				47.01		100.2832

				47.03		100.2832

				47.05		100.2832

				47.07		100.2832

				47.09		100.2832

				47.11		100.2832

				47.13		100.2832

				47.15		100.2832

				47.17		100.2832

				47.19		100.2832

				47.21		100.2832

				47.23		100.2871

				47.25		100.2871

				47.27		100.2871

				47.28		100.2871

				47.3		100.2871

				47.32		100.2871

				47.34		100.2871

				47.36		100.2871

				47.38		100.2871

				47.4		100.2871

				47.42		100.2871

				47.44		100.2871

				47.46		100.2871

				47.48		100.2871

				47.5		100.2871

				47.52		100.2871

				47.54		100.2871

				47.56		100.2871

				47.58		100.2871

				47.6		100.2871

				47.62		100.2871

				47.63		100.2871

				47.65		100.2871

				47.67		100.291

				47.69		100.291

				47.71		100.291

				47.73		100.291

				47.75		100.291

				47.77		100.291

				47.79		100.291

				47.81		100.291

				47.83		100.291

				47.85		100.291

				47.87		100.291

				47.89		100.291

				47.91		100.291

				47.93		100.291

				47.95		100.291

				47.97		100.291

				47.99		100.291

				48.01		100.291

				48.02		100.291

				48.04		100.291

				48.06		100.291

				48.08		100.291

				48.1		100.2949

				48.12		100.2949

				48.14		100.2949

				48.16		100.2949

				48.18		100.2949

				48.2		100.2949

				48.22		100.2949

				48.24		100.2949

				48.26		100.2949

				48.28		100.2949

				48.3		100.2949

				48.32		100.2949

				48.34		100.2988

				48.36		100.2949

				48.38		100.2988

				48.4		100.2949

				48.42		100.2988

				48.44		100.2988

				48.46		100.2988

				48.47		100.2988

				48.49		100.2988

				48.51		100.2988

				48.53		100.2988

				48.55		100.2988

				48.57		100.2988

				48.59		100.2988

				48.61		100.2988

				48.63		100.2988

				48.65		100.2988

				48.67		100.2988

				48.69		100.2988

				48.71		100.2988

				48.73		100.2988

				48.75		100.2988

				48.77		100.2988

				48.79		100.2988

				48.81		100.3026

				48.83		100.2988

				48.85		100.3026

				48.87		100.3026

				48.89		100.3026

				48.91		100.3026

				48.93		100.3026

				48.95		100.3026

				48.97		100.3026

				48.99		100.3026

				49		100.3026

				49.02		100.3026

				49.04		100.3026

				49.06		100.3026

				49.08		100.3026

				49.1		100.3026

				49.12		100.3026

				49.14		100.3026

				49.16		100.3026

				49.18		100.3026

				49.2		100.3026

				49.22		100.3026

				49.24		100.3026

				49.26		100.3026

				49.28		100.3026

				49.3		100.3026

				49.32		100.3026

				49.34		100.3026

				49.36		100.3026

				49.38		100.3026

				49.4		100.3026

				49.42		100.3026

				49.44		100.3065

				49.46		100.3026

				49.48		100.3026

				49.5		100.3026

				49.52		100.3026

				49.54		100.3026

				49.56		100.3026

				49.58		100.3026

				49.6		100.3026

				49.62		100.3026

				49.64		100.3026

				49.66		100.3026

				49.68		100.3026

				49.7		100.3026

				49.72		100.3026

				49.74		100.3026

				49.76		100.3026

				49.78		100.3026

				49.8		100.3026

				49.81		100.3026

				49.83		100.3026

				49.85		100.3026

				49.87		100.3026

				49.89		100.3026

				49.91		100.3026

				49.93		100.3026

				49.95		100.3026

				49.97		100.3026

				49.99		100.3026

				50.01		100.3026

				50.03		100.3026

				50.05		100.3026

				50.07		100.3026

				50.09		100.3026

				50.11		100.3026

				50.13		100.3026

				50.15		100.3026

				50.17		100.3026

				50.19		100.3026

				50.21		100.3026

				50.23		100.3026

				50.25		100.3026

				50.27		100.3026

				50.29		100.3026

				50.31		100.3026

				50.33		100.3026

				50.35		100.3026

				50.37		100.3026

				50.39		100.3026

				50.41		100.3026

				50.43		100.3026

				50.45		100.3026

				50.47		100.3026

				50.49		100.3026

				50.51		100.3065

				50.53		100.3026

				50.55		100.3065

				50.57		100.3026

				50.59		100.3026

				50.61		100.3026

				50.63		100.3065

				50.65		100.3065

				50.67		100.3065

				50.69		100.3026

				50.71		100.3065

				50.73		100.3065

				50.75		100.3065

				50.77		100.3065

				50.79		100.3065

				50.81		100.3065

				50.83		100.3065

				50.85		100.3065

				50.87		100.3065

				50.89		100.3065

				50.91		100.3065

				50.93		100.3065

				50.95		100.3065

				50.97		100.3065

				50.99		100.3065

				51.01		100.3065

				51.03		100.3104

				51.05		100.3065

				51.07		100.3104

				51.09		100.3104

				51.11		100.3104

				51.13		100.3104

				51.15		100.3104

				51.17		100.3104

				51.19		100.3104

				51.21		100.3104

				51.23		100.3104

				51.25		100.3104

				51.27		100.3104

				51.29		100.3104

				51.31		100.3104

				51.33		100.3104

				51.35		100.3143

				51.37		100.3104

				51.39		100.3143

				51.41		100.3143

				51.43		100.3143

				51.45		100.3143

				51.47		100.3143

				51.49		100.3143

				51.51		100.3143

				51.53		100.3143

				51.55		100.3143

				51.57		100.3143

				51.59		100.3143

				51.61		100.3143

				51.63		100.3143

				51.65		100.3182

				51.67		100.3143

				51.69		100.3182

				51.71		100.3182

				51.73		100.3182

				51.75		100.3182

				51.77		100.3182

				51.79		100.3182

				51.81		100.3182

				51.83		100.3182

				51.85		100.3182

				51.87		100.3182

				51.89		100.3182

				51.91		100.3182

				51.93		100.3182

				51.95		100.3182

				51.97		100.3182

				51.99		100.3182

				52.01		100.3182

				52.03		100.3182

				52.05		100.3182

				52.07		100.3182

				52.09		100.3182

				52.11		100.3182

				52.13		100.3182

				52.15		100.3182

				52.17		100.3182

				52.19		100.3182

				52.21		100.3182

				52.23		100.3182

				52.25		100.322

				52.27		100.3182

				52.29		100.322

				52.31		100.322

				52.33		100.322

				52.35		100.322

				52.37		100.322

				52.39		100.322

				52.41		100.322

				52.43		100.322

				52.45		100.322

				52.47		100.3182

				52.49		100.322

				52.51		100.3182

				52.53		100.322

				52.55		100.3182

				52.57		100.3182

				52.59		100.322

				52.61		100.3182

				52.63		100.3182

				52.65		100.3182

				52.67		100.3182

				52.69		100.3182

				52.71		100.3182

				52.73		100.322

				52.75		100.322

				52.77		100.3182

				52.79		100.3182

				52.81		100.322

				52.83		100.3182

				52.85		100.322

				52.87		100.3182

				52.89		100.322

				52.91		100.322

				52.93		100.322

				52.95		100.3182

				52.97		100.3182

				52.99		100.3182

				53.01		100.3182

				53.03		100.3182

				53.05		100.3182

				53.07		100.3182

				53.09		100.3182

				53.11		100.3182

				53.13		100.3182

				53.15		100.3182

				53.17		100.3182

				53.2		100.3182

				53.22		100.3182

				53.24		100.3182

				53.26		100.3182

				53.28		100.3182

				53.3		100.3182

				53.32		100.3182

				53.34		100.3182

				53.36		100.3182

				53.38		100.3182

				53.4		100.3182

				53.42		100.3182

				53.44		100.3182

				53.46		100.3182

				53.48		100.3182

				53.5		100.3182

				53.52		100.3182

				53.54		100.3182

				53.56		100.3182

				53.58		100.3182

				53.6		100.3182

				53.62		100.3143

				53.64		100.3143

				53.66		100.3143

				53.68		100.3143

				53.7		100.3143

				53.72		100.3143

				53.74		100.3143

				53.76		100.3143

				53.78		100.3143

				53.8		100.3143

				53.82		100.3143

				53.84		100.3143

				53.86		100.3143

				53.88		100.3143

				53.9		100.3143

				53.92		100.3143

				53.94		100.3143

				53.96		100.3143

				53.98		100.3143

				54		100.3143

				54.02		100.3143

				54.04		100.3143

				54.07		100.3143

				54.09		100.3143

				54.11		100.3143

				54.13		100.3143

				54.15		100.3143

				54.17		100.3143

				54.19		100.3182

				54.21		100.3143

				54.23		100.3182

				54.25		100.3182

				54.27		100.3182

				54.29		100.3143

				54.31		100.3182

				54.33		100.3182

				54.35		100.3143

				54.37		100.3143

				54.39		100.3143

				54.41		100.3143

				54.43		100.3143

				54.45		100.3143

				54.47		100.3182

				54.49		100.3182

				54.51		100.3182

				54.53		100.3182

				54.55		100.3182

				54.57		100.3182

				54.59		100.3182

				54.61		100.3182

				54.63		100.3182

				54.65		100.3182

				54.67		100.3182

				54.69		100.3182

				54.71		100.3182

				54.74		100.3182

				54.76		100.3182

				54.78		100.3182

				54.8		100.322

				54.82		100.3182

				54.84		100.322

				54.86		100.3182

				54.88		100.3182

				54.9		100.3182

				54.92		100.3182

				54.94		100.3182

				54.96		100.3182

				54.98		100.3182

				55		100.322

				55.02		100.322

				55.04		100.322

				55.06		100.322

				55.08		100.322

				55.1		100.322

				55.12		100.322

				55.14		100.322

				55.16		100.322

				55.18		100.322

				55.2		100.322

				55.22		100.322

				55.24		100.322

				55.26		100.322

				55.28		100.3259

				55.31		100.322

				55.33		100.322

				55.35		100.322

				55.37		100.322

				55.39		100.322

				55.41		100.322

				55.43		100.322

				55.45		100.322

				55.47		100.322

				55.49		100.322

				55.51		100.322

				55.53		100.322

				55.55		100.3259

				55.57		100.3259

				55.59		100.3259

				55.61		100.3259

				55.63		100.3259

				55.65		100.3259

				55.67		100.3259

				55.69		100.3259

				55.71		100.3259

				55.73		100.3259

				55.75		100.3298

				55.77		100.3298

				55.79		100.3298

				55.81		100.3298

				55.84		100.3298

				55.86		100.3298

				55.88		100.3298

				55.9		100.3298

				55.92		100.3298

				55.94		100.3298

				55.96		100.3298

				55.98		100.3298

				56		100.3298

				56.02		100.3298

				56.04		100.3298

				56.06		100.3298

				56.08		100.3298

				56.1		100.3298

				56.12		100.3298

				56.14		100.3298

				56.16		100.3298

				56.18		100.3298

				56.2		100.3298

				56.22		100.3298

				56.24		100.3298

				56.26		100.3298

				56.28		100.3298

				56.31		100.3298

				56.33		100.3298

				56.35		100.3298

				56.37		100.3298

				56.39		100.3298

				56.41		100.3298

				56.43		100.3337

				56.45		100.3337

				56.47		100.3337

				56.49		100.3298

				56.51		100.3337

				56.53		100.3337

				56.55		100.3337

				56.57		100.3337

				56.59		100.3337

				56.61		100.3337

				56.63		100.3337

				56.65		100.3337

				56.67		100.3337

				56.69		100.3337

				56.71		100.3337

				56.73		100.3337

				56.76		100.3337

				56.78		100.3337

				56.8		100.3337

				56.82		100.3337

				56.84		100.3337

				56.86		100.3337

				56.88		100.3337

				56.9		100.3337

				56.92		100.3337

				56.94		100.3337

				56.96		100.3337

				56.98		100.3376

				57		100.3376

				57.02		100.3337

				57.04		100.3337

				57.06		100.3376

				57.08		100.3376

				57.1		100.3376

				57.12		100.3376

				57.14		100.3376

				57.17		100.3376

				57.19		100.3376

				57.21		100.3376

				57.23		100.3376

				57.25		100.3376

				57.27		100.3376

				57.29		100.3376

				57.31		100.3376

				57.33		100.3337

				57.35		100.3376

				57.37		100.3376

				57.39		100.3376

				57.41		100.3376

				57.43		100.3376

				57.45		100.3376

				57.47		100.3376

				57.49		100.3414

				57.51		100.3414

				57.53		100.3414

				57.56		100.3414

				57.58		100.3414

				57.6		100.3414

				57.62		100.3414

				57.64		100.3414

				57.66		100.3414

				57.68		100.3414

				57.7		100.3376

				57.72		100.3376

				57.74		100.3376

				57.76		100.3376

				57.78		100.3376

				57.8		100.3376

				57.82		100.3376

				57.84		100.3376

				57.86		100.3376

				57.88		100.3376

				57.9		100.3376

				57.93		100.3376

				57.95		100.3376

				57.97		100.3414

				57.99		100.3376

				58.01		100.3376

				58.03		100.3376

				58.05		100.3376

				58.07		100.3376

				58.09		100.3376

				58.11		100.3376

				58.13		100.3376

				58.15		100.3376

				58.17		100.3376

				58.19		100.3376

				58.21		100.3376

				58.23		100.3376

				58.25		100.3376

				58.27		100.3337

				58.3		100.3376

				58.32		100.3376

				58.34		100.3376

				58.36		100.3376

				58.38		100.3376

				58.4		100.3376

				58.42		100.3376

				58.44		100.3376

				58.46		100.3376

				58.48		100.3376

				58.5		100.3376

				58.52		100.3376

				58.54		100.3376

				58.56		100.3376

				58.58		100.3376

				58.6		100.3376

				58.62		100.3376

				58.64		100.3376

				58.67		100.3376

				58.69		100.3376

				58.71		100.3376

				58.73		100.3376

				58.75		100.3376

				58.77		100.3376

				58.79		100.3376

				58.81		100.3376

				58.83		100.3376

				58.85		100.3376

				58.87		100.3376

				58.89		100.3414

				58.91		100.3414

				58.93		100.3414

				58.95		100.3414

				58.97		100.3414

				58.99		100.3414

				59.02		100.3414

				59.04		100.3414

				59.06		100.3414

				59.08		100.3414

				59.1		100.3414

				59.12		100.3414

				59.14		100.3414

				59.16		100.3414

				59.18		100.3414

				59.2		100.3414

				59.22		100.3414

				59.24		100.3414

				59.26		100.3414

				59.28		100.3414

				59.3		100.3414

				59.32		100.3414

				59.35		100.3414

				59.37		100.3414

				59.39		100.3414

				59.41		100.3414

				59.43		100.3414

				59.45		100.3414

				59.47		100.3414

				59.49		100.3453

				59.51		100.3453

				59.53		100.3414

				59.55		100.3453

				59.57		100.3453

				59.59		100.3453

				59.61		100.3453

				59.63		100.3453

				59.65		100.3453

				59.68		100.3453

				59.7		100.3453

				59.72		100.3453

				59.74		100.3453

				59.76		100.3453

				59.78		100.3453

				59.8		100.3453

				59.82		100.3492

				59.84		100.3492

				59.86		100.3492

				59.88		100.3492

				59.9		100.3492

				59.92		100.3492

				59.94		100.3492

				59.96		100.3492

				59.98		100.3492

				60		100.3492

				60.03		100.3492

				60.05		100.3492

				60.07		100.3531

				60.09		100.3531

				60.11		100.3531

				60.13		100.3531

				60.15		100.3531

				60.17		100.3531

				60.19		100.3531

				60.21		100.3531

				60.23		100.357

				60.25		100.357

				60.27		100.357

				60.29		100.357

				60.31		100.357

				60.33		100.357

				60.35		100.357

				60.38		100.357

				60.4		100.357

				60.42		100.357

				60.44		100.357

				60.46		100.357

				60.48		100.357

				60.5		100.357

				60.52		100.357

				60.54		100.357

				60.56		100.357

				60.58		100.357

				60.6		100.357

				60.62		100.357

				60.64		100.357

				60.66		100.357

				60.68		100.357

				60.7		100.3608

				60.72		100.357

				60.75		100.3608

				60.77		100.3608

				60.79		100.3608

				60.81		100.3608

				60.83		100.3608

				60.85		100.3608

				60.87		100.3608

				60.89		100.3608

				60.91		100.3608

				60.93		100.3608

				60.95		100.3608

				60.97		100.3608

				60.99		100.3608

				61.01		100.3608

				61.03		100.3608

				61.05		100.3608

				61.07		100.3608

				61.09		100.3608

				61.12		100.3647

				61.14		100.3608

				61.16		100.3647

				61.18		100.3647

				61.2		100.3647

				61.22		100.3647

				61.24		100.3647

				61.26		100.3647

				61.28		100.3647

				61.3		100.3647

				61.32		100.3647

				61.34		100.3647

				61.36		100.3647

				61.38		100.3647

				61.4		100.3647

				61.42		100.3647

				61.44		100.3647

				61.46		100.3647

				61.48		100.3647

				61.51		100.3647

				61.53		100.3647

				61.55		100.3647

				61.57		100.3647

				61.59		100.3647

				61.61		100.3647

				61.63		100.3647

				61.65		100.3647

				61.67		100.3686

				61.69		100.3647

				61.71		100.3686

				61.73		100.3686

				61.75		100.3686

				61.77		100.3686

				61.79		100.3686

				61.81		100.3686

				61.83		100.3686

				61.85		100.3686

				61.87		100.3686

				61.9		100.3686

				61.92		100.3686

				61.94		100.3686

				61.96		100.3686

				61.98		100.3686

				62		100.3686

				62.02		100.3686

				62.04		100.3686

				62.06		100.3686

				62.08		100.3686

				62.1		100.3686

				62.12		100.3686

				62.14		100.3686

				62.16		100.3686

				62.18		100.3686

				62.2		100.3686

				62.22		100.3686

				62.24		100.3686

				62.26		100.3686

				62.28		100.3686

				62.31		100.3647

				62.33		100.3686

				62.35		100.3725

				62.37		100.3686

				62.39		100.3686

				62.41		100.3725

				62.43		100.3725

				62.45		100.3725

				62.47		100.3725

				62.49		100.3686

				62.51		100.3725

				62.53		100.3686

				62.55		100.3725

				62.57		100.3725

				62.59		100.3725

				62.61		100.3725

				62.63		100.3725

				62.65		100.3725

				62.67		100.3725

				62.69		100.3725

				62.71		100.3725

				62.74		100.3725

				62.76		100.3725

				62.78		100.3725

				62.8		100.3725

				62.82		100.3725

				62.84		100.3725

				62.86		100.3725

				62.88		100.3725

				62.9		100.3686

				62.92		100.3686

				62.94		100.3686

				62.96		100.3686

				62.98		100.3686

				63		100.3686

				63.02		100.3686

				63.04		100.3686

				63.06		100.3686

				63.08		100.3686

				63.1		100.3686

				63.12		100.3686

				63.14		100.3686

				63.17		100.3686

				63.19		100.3686

				63.21		100.3686

				63.23		100.3686

				63.25		100.3686

				63.27		100.3686

				63.29		100.3686

				63.31		100.3686

				63.33		100.3686

				63.35		100.3686

				63.37		100.3686

				63.39		100.3686

				63.41		100.3686

				63.43		100.3686

				63.45		100.3686

				63.47		100.3686

				63.49		100.3686

				63.51		100.3686

				63.53		100.3686

				63.55		100.3686

				63.58		100.3686

				63.6		100.3686

				63.62		100.3686

				63.64		100.3686

				63.66		100.3686

				63.68		100.3686

				63.7		100.3686

				63.72		100.3686

				63.74		100.3686

				63.76		100.3686

				63.78		100.3686

				63.8		100.3686

				63.82		100.3686

				63.84		100.3686

				63.86		100.3686

				63.88		100.3686

				63.9		100.3686

				63.92		100.3686

				63.94		100.3686

				63.96		100.3686

				63.98		100.3686

				64.01		100.3686

				64.03		100.3686

				64.05		100.3686

				64.07		100.3686

				64.09		100.3686

				64.11		100.3686

				64.13		100.3686

				64.15		100.3686

				64.17		100.3686

				64.19		100.3686

				64.21		100.3686

				64.23		100.3686

				64.25		100.3686

				64.27		100.3686

				64.29		100.3686

				64.31		100.3686

				64.33		100.3725

				64.35		100.3686

				64.37		100.3686

				64.39		100.3725

				64.42		100.3686

				64.44		100.3725

				64.46		100.3725

				64.48		100.3725

				64.5		100.3725

				64.52		100.3725

				64.54		100.3725

				64.56		100.3725

				64.58		100.3725

				64.6		100.3725

				64.62		100.3725

				64.64		100.3725

				64.66		100.3725

				64.68		100.3725

				64.7		100.3725

				64.72		100.3725

				64.74		100.3725

				64.76		100.3725

				64.78		100.3725

				64.8		100.3725

				64.83		100.3725

				64.85		100.3725

				64.87		100.3725

				64.89		100.3725

				64.91		100.3725

				64.93		100.3725

				64.95		100.3764

				64.97		100.3764

				64.99		100.3764

				65.01		100.3764

				65.03		100.3764

				65.05		100.3764

				65.07		100.3764

				65.09		100.3764

				65.11		100.3764

				65.13		100.3764

				65.15		100.3764

				65.17		100.3764

				65.19		100.3764

				65.22		100.3764

				65.24		100.3764

				65.26		100.3764

				65.28		100.3764

				65.3		100.3764

				65.32		100.3764

				65.34		100.3764

				65.36		100.3764

				65.38		100.3764

				65.4		100.3764

				65.42		100.3764

				65.44		100.3764

				65.46		100.3764

				65.48		100.3764

				65.5		100.3764

				65.52		100.3764

				65.54		100.3764

				65.56		100.3764

				65.58		100.3764

				65.61		100.3764

				65.63		100.3764

				65.65		100.3764

				65.67		100.3764

				65.69		100.3764

				65.71		100.3764

				65.73		100.3764

				65.75		100.3764

				65.77		100.3764

				65.79		100.3764

				65.81		100.3764

				65.83		100.3764

				65.85		100.3764

				65.87		100.3764

				65.89		100.3764

				65.91		100.3764

				65.93		100.3764

				65.95		100.3764

				65.98		100.3764

				66		100.3764

				66.02		100.3764

				66.04		100.3764

				66.06		100.3764

				66.08		100.3764

				66.1		100.3764

				66.12		100.3764

				66.14		100.3764

				66.16		100.3764

				66.18		100.3764

				66.2		100.3764

				66.22		100.3764

				66.24		100.3764

				66.26		100.3764

				66.28		100.3764

				66.3		100.3764

				66.32		100.3764

				66.35		100.3764

				66.37		100.3764

				66.39		100.3764

				66.41		100.3764

				66.43		100.3764

				66.45		100.3764

				66.47		100.3725

				66.49		100.3725

				66.51		100.3725

				66.53		100.3725

				66.55		100.3725

				66.57		100.3725

				66.59		100.3725

				66.61		100.3725

				66.63		100.3725

				66.65		100.3725

				66.67		100.3725

				66.7		100.3725

				66.72		100.3725

				66.74		100.3725

				66.76		100.3725

				66.78		100.3725

				66.8		100.3725

				66.82		100.3725

				66.84		100.3725

				66.86		100.3725

				66.88		100.3725

				66.9		100.3725

				66.92		100.3725

				66.94		100.3725

				66.96		100.3725

				66.98		100.3725

				67		100.3725

				67.02		100.3725

				67.05		100.3725

				67.07		100.3725

				67.09		100.3725

				67.11		100.3725

				67.13		100.3725

				67.15		100.3725

				67.17		100.3725

				67.19		100.3725

				67.21		100.3725

				67.23		100.3725

				67.25		100.3725

				67.27		100.3725

				67.29		100.3725

				67.31		100.3725

				67.33		100.3725

				67.35		100.3725

				67.38		100.3725

				67.4		100.3725

				67.42		100.3725

				67.44		100.3725

				67.46		100.3725

				67.48		100.3725

				67.5		100.3725

				67.52		100.3764

				67.54		100.3725

				67.56		100.3725

				67.58		100.3725

				67.6		100.3725

				67.62		100.3764

				67.64		100.3764

				67.66		100.3725

				67.69		100.3725

				67.71		100.3725

				67.73		100.3725

				67.75		100.3725

				67.77		100.3725

				67.79		100.3725

				67.81		100.3725

				67.83		100.3725

				67.85		100.3725

				67.87		100.3725

				67.89		100.3725

				67.91		100.3725

				67.93		100.3725

				67.95		100.3725

				67.97		100.3725

				68		100.3725

				68.02		100.3725

				68.04		100.3725

				68.06		100.3725

				68.08		100.3725

				68.1		100.3725

				68.12		100.3725

				68.14		100.3725

				68.16		100.3725

				68.18		100.3725

				68.2		100.3725

				68.22		100.3725

				68.24		100.3725

				68.26		100.3725

				68.28		100.3764

				68.31		100.3764

				68.33		100.3764

				68.35		100.3764

				68.37		100.3764

				68.39		100.3764

				68.41		100.3764

				68.43		100.3764

				68.45		100.3764

				68.47		100.3764

				68.49		100.3764

				68.51		100.3764

				68.53		100.3764

				68.55		100.3764

				68.57		100.3764

				68.6		100.3764

				68.62		100.3764

				68.64		100.3764

				68.66		100.3764

				68.68		100.3764

				68.7		100.3764

				68.72		100.3764

				68.74		100.3764

				68.76		100.3802

				68.78		100.3764

				68.8		100.3764

				68.82		100.3802

				68.84		100.3764

				68.86		100.3802

				68.89		100.3802

				68.91		100.3802

				68.93		100.3802

				68.95		100.3764

				68.97		100.3764

				68.99		100.3764

				69.01		100.3802

				69.03		100.3764

				69.05		100.3764

				69.07		100.3802

				69.09		100.3764

				69.11		100.3764

				69.13		100.3764

				69.16		100.3764

				69.18		100.3764

				69.2		100.3764

				69.22		100.3764

				69.24		100.3764

				69.26		100.3764

				69.28		100.3764

				69.3		100.3764

				69.32		100.3764

				69.34		100.3764

				69.36		100.3764

				69.38		100.3802

				69.4		100.3802

				69.42		100.3764

				69.45		100.3802

				69.47		100.3764

				69.49		100.3764

				69.51		100.3764

				69.53		100.3764

				69.55		100.3764

				69.57		100.3764

				69.59		100.3764

				69.61		100.3764

				69.63		100.3764

				69.65		100.3764

				69.67		100.3764

				69.7		100.3764

				69.72		100.3764

				69.74		100.3764

				69.76		100.3764

				69.78		100.3764

				69.8		100.3764

				69.82		100.3764

				69.84		100.3764

				69.86		100.3764

				69.88		100.3764

				69.9		100.3764

				69.92		100.3764

				69.94		100.3802

				69.97		100.3802

				69.99		100.3802

				70.01		100.3802

				70.03		100.3764

				70.05		100.3802

				70.07		100.3802

				70.09		100.3802

				70.11		100.3802

				70.13		100.3802

				70.15		100.3802

				70.17		100.3764

				70.19		100.3764

				70.22		100.3802

				70.24		100.3802

				70.26		100.3802

				70.28		100.3802

				70.3		100.3802

				70.32		100.3802

				70.34		100.3802

				70.36		100.3802

				70.38		100.3802

				70.4		100.3802

				70.42		100.3802

				70.44		100.3802

				70.46		100.3802

				70.49		100.3802

				70.51		100.3802

				70.53		100.3802

				70.55		100.3802

				70.57		100.3802

				70.59		100.3802

				70.61		100.3802

				70.63		100.3802

				70.65		100.3802

				70.67		100.3802

				70.69		100.3802

				70.71		100.3802

				70.74		100.3802

				70.76		100.3802

				70.78		100.3802

				70.8		100.3802

				70.82		100.3802

				70.84		100.3802

				70.86		100.3841

				70.88		100.3802

				70.9		100.3841

				70.92		100.3802

				70.94		100.3841

				70.96		100.3802

				70.99		100.3802

				71.01		100.3802

				71.03		100.3802

				71.05		100.3802

				71.07		100.3802

				71.09		100.3802

				71.11		100.3802

				71.13		100.3802

				71.15		100.3802

				71.17		100.3802

				71.19		100.3802

				71.21		100.3802

				71.24		100.3802

				71.26		100.3802

				71.28		100.3802

				71.3		100.3802

				71.32		100.3802

				71.34		100.3802

				71.36		100.3802

				71.38		100.3802

				71.4		100.3802

				71.42		100.3802

				71.44		100.3802

				71.47		100.3802

				71.49		100.3802

				71.51		100.3802

				71.53		100.3802

				71.55		100.3802

				71.57		100.3802

				71.59		100.3802

				71.61		100.3802

				71.63		100.3802

				71.65		100.3802

				71.67		100.3802

				71.7		100.3802

				71.72		100.3802

				71.74		100.3802

				71.76		100.3802

				71.78		100.3802

				71.8		100.3802

				71.82		100.3841

				71.84		100.3841

				71.86		100.3841

				71.88		100.3841

				71.9		100.3841

				71.92		100.3841

				71.95		100.3841

				71.97		100.3841

				71.99		100.3841

				72.01		100.3841

				72.03		100.3841

				72.05		100.3841

				72.07		100.3841

				72.09		100.3841

				72.11		100.3841

				72.13		100.3841

				72.15		100.3841

				72.18		100.3802

				72.2		100.3841

				72.22		100.3841

				72.24		100.3841

				72.26		100.3841

				72.28		100.3841

				72.3		100.3841

				72.32		100.3841

				72.34		100.3841

				72.36		100.3802

				72.38		100.3802

				72.41		100.3802

				72.43		100.3802

				72.45		100.3802

				72.47		100.3802

				72.49		100.3802

				72.51		100.3802

				72.53		100.3802

				72.55		100.3802

				72.57		100.3802

				72.59		100.3802

				72.61		100.3802

				72.64		100.3802

				72.66		100.3802

				72.68		100.3802

				72.7		100.3802

				72.72		100.3802

				72.74		100.3802

				72.76		100.3802

				72.78		100.3802

				72.8		100.3802

				72.82		100.3802

				72.84		100.3802

				72.87		100.3802

				72.89		100.3802

				72.91		100.3802

				72.93		100.3802

				72.95		100.3802

				72.97		100.3802

				72.99		100.3802

				73.01		100.3802

				73.03		100.3802

				73.05		100.3802

				73.08		100.3802

				73.1		100.3802

				73.12		100.3802

				73.14		100.3802

				73.16		100.3802

				73.18		100.3802

				73.2		100.3841

				73.22		100.3802

				73.24		100.3841

				73.26		100.3841

				73.28		100.3841

				73.31		100.3841

				73.33		100.3841

				73.35		100.3841

				73.37		100.3841

				73.39		100.3841

				73.41		100.3841

				73.43		100.3841

				73.45		100.3841

				73.47		100.3841

				73.49		100.3841

				73.52		100.3841

				73.54		100.3841

				73.56		100.3841

				73.58		100.3841

				73.6		100.3841

				73.62		100.3841

				73.64		100.3841

				73.66		100.3841

				73.68		100.3841

				73.7		100.3841

				73.72		100.3841

				73.75		100.3841

				73.77		100.3841

				73.79		100.3841

				73.81		100.3841

				73.83		100.3841

				73.85		100.3841

				73.87		100.3841

				73.89		100.3841

				73.91		100.3841

				73.93		100.3841

				73.96		100.3841

				73.98		100.3841

				74		100.3841

				74.02		100.3841

				74.04		100.3841

				74.06		100.3802

				74.08		100.3841

				74.1		100.3841

				74.12		100.3841

				74.14		100.3841

				74.17		100.3841

				74.19		100.3841

				74.21		100.3841

				74.23		100.3841

				74.25		100.3841

				74.27		100.3841

				74.29		100.3841

				74.31		100.3841

				74.33		100.3841

				74.35		100.3841

				74.38		100.3841

				74.4		100.3841

				74.42		100.3841

				74.44		100.3841

				74.46		100.3841

				74.48		100.3841

				74.5		100.3841

				74.52		100.3841

				74.54		100.3841

				74.56		100.3841

				74.59		100.3841

				74.61		100.3841

				74.63		100.388

				74.65		100.388

				74.67		100.388

				74.69		100.388

				74.71		100.388

				74.73		100.388

				74.75		100.388

				74.77		100.388

				74.79		100.388

				74.82		100.388

				74.84		100.388

				74.86		100.388

				74.88		100.388

				74.9		100.388

				74.92		100.388

				74.94		100.388

				74.96		100.388

				74.98		100.388

				75		100.388

				75.03		100.3919

				75.05		100.3919

				75.07		100.3919

				75.09		100.388

				75.11		100.3919

				75.13		100.3919

				75.15		100.3919

				75.17		100.3919

				75.19		100.3919

				75.21		100.3919

				75.24		100.3919

				75.26		100.3919

				75.28		100.3919

				75.3		100.3919

				75.32		100.3919

				75.34		100.3919

				75.36		100.3919

				75.38		100.3919

				75.4		100.3919

				75.42		100.3919

				75.45		100.3919

				75.47		100.3919

				75.49		100.3919

				75.51		100.3919

				75.53		100.3919

				75.55		100.3919

				75.57		100.3919

				75.59		100.3919

				75.61		100.3919

				75.64		100.3919

				75.66		100.3919

				75.68		100.3958

				75.7		100.3919

				75.72		100.3919

				75.74		100.3958

				75.76		100.3958

				75.78		100.3919

				75.8		100.3919

				75.82		100.3919

				75.85		100.3919

				75.87		100.3919

				75.89		100.3958

				75.91		100.3958

				75.93		100.3958

				75.95		100.3958

				75.97		100.3958

				75.99		100.3958

				76.01		100.3958

				76.03		100.3958

				76.06		100.3958

				76.08		100.3958

				76.1		100.3958

				76.12		100.3958

				76.14		100.3958

				76.16		100.3958

				76.18		100.3958

				76.2		100.3958

				76.22		100.3958

				76.24		100.3958

				76.27		100.3958

				76.29		100.3958

				76.31		100.3958

				76.33		100.3958

				76.35		100.3958

				76.37		100.3958

				76.39		100.3958

				76.41		100.3958

				76.43		100.3958

				76.46		100.3958

				76.48		100.3958

				76.5		100.3958

				76.52		100.3958

				76.54		100.3958

				76.56		100.3958

				76.58		100.3958

				76.6		100.3958

				76.62		100.3958

				76.64		100.3958

				76.67		100.3958

				76.69		100.3958

				76.71		100.3958

				76.73		100.3958

				76.75		100.3958

				76.77		100.3958

				76.79		100.3958

				76.81		100.3958

				76.83		100.3958

				76.85		100.3958

				76.88		100.3958

				76.9		100.3958

				76.92		100.3919

				76.94		100.3919

				76.96		100.3919

				76.98		100.3919

				77		100.3919

				77.02		100.3919

				77.04		100.3919

				77.06		100.3919

				77.09		100.3919

				77.11		100.3919

				77.13		100.3919

				77.15		100.3919

				77.17		100.3919

				77.19		100.3919

				77.21		100.3919

				77.23		100.3919

				77.25		100.3919

				77.28		100.3919

				77.3		100.3919

				77.32		100.3919

				77.34		100.3919

				77.36		100.3919

				77.38		100.3919

				77.4		100.3919

				77.42		100.3919

				77.44		100.3919

				77.46		100.3919

				77.49		100.3919

				77.51		100.3919

				77.53		100.3919

				77.55		100.3919

				77.57		100.3919

				77.59		100.3919

				77.61		100.3919

				77.63		100.3919

				77.65		100.3919

				77.67		100.3919

				77.7		100.3919

				77.72		100.3919

				77.74		100.3919

				77.76		100.3919

				77.78		100.3919

				77.8		100.3919

				77.82		100.3919

				77.84		100.3919

				77.86		100.3919

				77.89		100.3919

				77.91		100.3919

				77.93		100.3919

				77.95		100.3919

				77.97		100.3919

				77.99		100.3919

				78.01		100.3919

				78.03		100.3919

				78.05		100.3919

				78.07		100.3919

				78.1		100.3919

				78.12		100.3919

				78.14		100.388

				78.16		100.388

				78.18		100.388

				78.2		100.388

				78.22		100.388

				78.24		100.388

				78.26		100.3919

				78.28		100.3919

				78.31		100.3919

				78.33		100.3919

				78.35		100.3919

				78.37		100.3919

				78.39		100.3919

				78.41		100.3919

				78.43		100.3919

				78.45		100.3919

				78.47		100.3919

				78.5		100.3919

				78.52		100.3919

				78.54		100.3919

				78.56		100.3919

				78.58		100.3919

				78.6		100.3919

				78.62		100.3919

				78.64		100.3919

				78.66		100.3919

				78.68		100.3919

				78.71		100.3919

				78.73		100.3919

				78.75		100.3919

				78.77		100.3919

				78.79		100.3919

				78.81		100.3919

				78.83		100.3919

				78.85		100.3919

				78.87		100.3919

				78.9		100.3919

				78.92		100.3919

				78.94		100.3919

				78.96		100.3919

				78.98		100.3919

				79		100.3919

				79.02		100.3919

				79.04		100.3919

				79.06		100.3919

				79.09		100.3919

				79.11		100.3919

				79.13		100.3919

				79.15		100.3919

				79.17		100.3919

				79.19		100.3919

				79.21		100.3958

				79.23		100.3958

				79.25		100.3958

				79.27		100.3958

				79.3		100.3958

				79.32		100.3958

				79.34		100.3958

				79.36		100.3958

				79.38		100.3958

				79.4		100.3958

				79.42		100.3958

				79.44		100.3958

				79.46		100.3958

				79.49		100.3958

				79.51		100.3958

				79.53		100.3958

				79.55		100.3958

				79.57		100.3958

				79.59		100.3958

				79.61		100.3958

				79.63		100.3958

				79.65		100.3958

				79.67		100.3958

				79.7		100.3958

				79.72		100.3958

				79.74		100.3958

				79.76		100.3958

				79.78		100.3958

				79.8		100.3958

				79.82		100.3958

				79.84		100.3958

				79.86		100.3958

				79.89		100.3958

				79.91		100.3958

				79.93		100.3958

				79.95		100.3958

				79.97		100.3958

				79.99		100.3958

				80.01		100.3958

				80.03		100.3958

				80.05		100.3996

				80.08		100.3996

				80.1		100.3996

				80.12		100.3996

				80.14		100.3996

				80.16		100.3996

				80.18		100.3996

				80.2		100.3996

				80.22		100.3996

				80.24		100.3996

				80.26		100.3996

				80.29		100.3996

				80.31		100.3996

				80.33		100.3996

				80.35		100.3996

				80.37		100.3996

				80.39		100.3996

				80.41		100.4035

				80.43		100.3996

				80.45		100.3996

				80.48		100.4035

				80.5		100.4035

				80.52		100.4035

				80.54		100.4035

				80.56		100.3996

				80.58		100.4035

				80.6		100.4035

				80.62		100.4035

				80.64		100.4035

				80.67		100.4035

				80.69		100.4035

				80.71		100.4035

				80.73		100.4035

				80.75		100.4035

				80.77		100.4035

				80.79		100.4035

				80.81		100.4035

				80.83		100.4035

				80.86		100.4035

				80.88		100.4035

				80.9		100.4035

				80.92		100.4035

				80.94		100.4035

				80.96		100.4035

				80.98		100.4035

				81		100.4035

				81.02		100.4035

				81.04		100.4035

				81.07		100.4035

				81.09		100.4035

				81.11		100.4035

				81.13		100.4035

				81.15		100.4035

				81.17		100.4035

				81.19		100.4035

				81.21		100.4035

				81.23		100.4035

				81.26		100.4035

				81.28		100.4035

				81.3		100.4035

				81.32		100.4035

				81.34		100.4035

				81.36		100.4035

				81.38		100.4035

				81.4		100.4035

				81.42		100.4035

				81.45		100.4035

				81.47		100.4035

				81.49		100.4035

				81.51		100.4035

				81.53		100.4035

				81.55		100.4035

				81.57		100.4035

				81.59		100.3996

				81.61		100.4035

				81.64		100.3996

				81.66		100.4035

				81.68		100.4035

				81.7		100.4035

				81.72		100.4035

				81.74		100.4035

				81.76		100.4035

				81.78		100.4035

				81.8		100.4035

				81.82		100.4035

				81.85		100.4035

				81.87		100.4035

				81.89		100.4035

				81.91		100.4035

				81.93		100.4035

				81.95		100.4035

				81.97		100.4035

				81.99		100.4035

				82.01		100.4035

				82.04		100.4035

				82.06		100.4035

				82.08		100.4035

				82.1		100.4035

				82.12		100.4035

				82.14		100.4035

				82.16		100.4035

				82.18		100.4035

				82.2		100.4035

				82.23		100.4035

				82.25		100.4035

				82.27		100.4035

				82.29		100.4035

				82.31		100.4035

				82.33		100.4035

				82.35		100.4035

				82.37		100.4035

				82.39		100.4035

				82.42		100.3996

				82.44		100.3996

				82.46		100.3996

				82.48		100.3996

				82.5		100.3996

				82.52		100.3996

				82.54		100.3996

				82.56		100.3996

				82.58		100.3996

				82.6		100.3996

				82.63		100.3996

				82.65		100.3996

				82.67		100.3996

				82.69		100.3996

				82.71		100.3996

				82.73		100.3996

				82.75		100.3996

				82.77		100.3996

				82.79		100.3996

				82.82		100.3996

				82.84		100.3996

				82.86		100.3996

				82.88		100.3996

				82.9		100.3996

				82.92		100.3996

				82.94		100.3996

				82.96		100.3996

				82.98		100.3996

				83.01		100.3996

				83.03		100.3996

				83.05		100.3996

				83.07		100.3996

				83.09		100.3996

				83.11		100.3996

				83.13		100.3996

				83.15		100.3996

				83.17		100.3996

				83.2		100.3996

				83.22		100.3996

				83.24		100.3996

				83.26		100.3996

				83.28		100.3996

				83.3		100.3996

				83.32		100.4035

				83.34		100.4035

				83.36		100.4035

				83.39		100.4035

				83.41		100.4035

				83.43		100.4035

				83.45		100.4035

				83.47		100.4035

				83.49		100.4035

				83.51		100.4035

				83.53		100.4035

				83.55		100.4035

				83.58		100.4035

				83.6		100.4035

				83.62		100.4035

				83.64		100.4035

				83.66		100.4035

				83.68		100.4035

				83.7		100.4035

				83.72		100.4035

				83.74		100.4035

				83.77		100.4035

				83.79		100.4035

				83.81		100.4035

				83.83		100.4035

				83.85		100.4035

				83.87		100.4035

				83.89		100.4035

				83.91		100.4035

				83.93		100.4035

				83.96		100.4035

				83.98		100.4035

				84		100.4035

				84.02		100.4035

				84.04		100.4035

				84.06		100.4035

				84.08		100.4035

				84.1		100.4035

				84.12		100.4035

				84.14		100.4035

				84.17		100.4035

				84.19		100.4035

				84.21		100.4035

				84.23		100.4035

				84.25		100.4035

				84.27		100.4035

				84.29		100.4035

				84.31		100.4035

				84.33		100.4035

				84.36		100.4035

				84.38		100.4035

				84.4		100.4035

				84.42		100.4035

				84.44		100.4035

				84.46		100.4035

				84.48		100.4035

				84.5		100.4035

				84.52		100.4035

				84.55		100.4035

				84.57		100.4035

				84.59		100.4035

				84.61		100.4035

				84.63		100.4074

				84.65		100.4074

				84.67		100.4074

				84.69		100.4074

				84.71		100.4074

				84.74		100.4074

				84.76		100.4074

				84.78		100.4074

				84.8		100.4074

				84.82		100.4074

				84.84		100.4074

				84.86		100.4074

				84.88		100.4074

				84.9		100.4074

				84.93		100.4074

				84.95		100.4074

				84.97		100.4035

				84.99		100.4035

				85.01		100.4035

				85.03		100.4035

				85.05		100.4035

				85.07		100.4035

				85.09		100.4035

				85.12		100.4035

				85.14		100.4035

				85.16		100.4035

				85.18		100.4035

				85.2		100.4035

				85.22		100.4035

				85.24		100.4035

				85.26		100.4035

				85.28		100.4035

				85.31		100.4035

				85.33		100.4035

				85.35		100.4035

				85.37		100.4074

				85.39		100.4035

				85.41		100.4035

				85.43		100.4074

				85.45		100.4035

				85.47		100.4074

				85.5		100.4035

				85.52		100.4074

				85.54		100.4035

				85.56		100.4035

				85.58		100.4035

				85.6		100.4035

				85.62		100.4035

				85.64		100.4035

				85.66		100.4035

				85.69		100.4035

				85.71		100.4035

				85.73		100.4035

				85.75		100.4035

				85.77		100.4035

				85.79		100.4035

				85.81		100.4035

				85.83		100.4035

				85.85		100.4035

				85.87		100.4035

				85.9		100.4035

				85.92		100.4035

				85.94		100.4035

				85.96		100.4035

				85.98		100.4035

				86		100.4035

				86.02		100.4035

				86.04		100.4035

				86.06		100.4035

				86.09		100.4035

				86.11		100.4035

				86.13		100.4035

				86.15		100.4035

				86.17		100.4035

				86.19		100.4035

				86.21		100.4035

				86.23		100.4035

				86.25		100.4035

				86.28		100.4035

				86.3		100.4074

				86.32		100.4074

				86.34		100.4074

				86.36		100.4074

				86.38		100.4074

				86.4		100.4074

				86.42		100.4074

				86.44		100.4074

				86.47		100.4074

				86.49		100.4074

				86.51		100.4074

				86.53		100.4074

				86.55		100.4074

				86.57		100.4074

				86.59		100.4074

				86.61		100.4074

				86.63		100.4074

				86.66		100.4074

				86.68		100.4074

				86.7		100.4074

				86.72		100.4074

				86.74		100.4074

				86.76		100.4074

				86.78		100.4074

				86.8		100.4074

				86.82		100.4074

				86.84		100.4074

				86.87		100.4074

				86.89		100.4074

				86.91		100.4074

				86.93		100.4074

				86.95		100.4074

				86.97		100.4074

				86.99		100.4074

				87.01		100.4074

				87.03		100.4074

				87.06		100.4074

				87.08		100.4113

				87.1		100.4113

				87.12		100.4113

				87.14		100.4113

				87.16		100.4113

				87.18		100.4113

				87.2		100.4074

				87.22		100.4113

				87.25		100.4113

				87.27		100.4113

				87.29		100.4113

				87.31		100.4113

				87.33		100.4113

				87.35		100.4113

				87.37		100.4113

				87.39		100.4113

				87.41		100.4113

				87.44		100.4113

				87.46		100.4113

				87.48		100.4113

				87.5		100.4113

				87.52		100.4113

				87.54		100.4113

				87.56		100.4113

				87.58		100.4113

				87.6		100.4074

				87.62		100.4113

				87.65		100.4113

				87.67		100.4113

				87.69		100.4113

				87.71		100.4113

				87.73		100.4113

				87.75		100.4113

				87.77		100.4113

				87.79		100.4113

				87.81		100.4113

				87.84		100.4113

				87.86		100.4113

				87.88		100.4113

				87.9		100.4113

				87.92		100.4113

				87.94		100.4113

				87.96		100.4113

				87.98		100.4113

				88		100.4113

				88.03		100.4113

				88.05		100.4113

				88.07		100.4113

				88.09		100.4113

				88.11		100.4113

				88.13		100.4113

				88.15		100.4113

				88.17		100.4113

				88.19		100.4113

				88.22		100.4113

				88.24		100.4113

				88.26		100.4113

				88.28		100.4113

				88.3		100.4152

				88.32		100.4113

				88.34		100.4152

				88.36		100.4113

				88.38		100.4113

				88.4		100.4113

				88.43		100.4113

				88.45		100.4113

				88.47		100.4113

				88.49		100.4113

				88.51		100.4113

				88.53		100.4113

				88.55		100.4113

				88.57		100.4113

				88.59		100.4113

				88.62		100.4113

				88.64		100.4113

				88.66		100.4113

				88.68		100.4113

				88.7		100.4113

				88.72		100.4113

				88.74		100.4113

				88.76		100.4152

				88.78		100.4113

				88.81		100.4113

				88.83		100.4113

				88.85		100.4152

				88.87		100.4113

				88.89		100.4113

				88.91		100.4152

				88.93		100.4152

				88.95		100.4113

				88.97		100.4113

				89		100.4152

				89.02		100.4152

				89.04		100.4152

				89.06		100.4152

				89.08		100.4152

				89.1		100.4152

				89.12		100.4152

				89.14		100.4152

				89.16		100.4152

				89.18		100.4152

				89.21		100.4152

				89.23		100.4152

				89.25		100.4152

				89.27		100.4152

				89.29		100.4152

				89.31		100.4152

				89.33		100.4152

				89.35		100.4152

				89.37		100.4152

				89.4		100.4152

				89.42		100.4152

				89.44		100.4152

				89.46		100.4152

				89.48		100.4152

				89.5		100.4152

				89.52		100.4152

				89.54		100.4152

				89.56		100.4152

				89.59		100.4152

				89.61		100.4152

				89.63		100.4152

				89.65		100.4152

				89.67		100.4152

				89.69		100.419

				89.71		100.4152

				89.73		100.4152

				89.75		100.4152

				89.78		100.419

				89.8		100.4152

				89.82		100.4152

				89.84		100.4152

				89.86		100.4152

				89.88		100.4152

				89.9		100.419

				89.92		100.4152

				89.94		100.4152

				89.96		100.4152

				89.99		100.4152

				90.01		100.4152

				90.03		100.419

				90.05		100.4152

				90.07		100.4152

				90.09		100.4152

				90.11		100.4152

				90.13		100.4152

				90.15		100.4152

				90.18		100.4152

				90.2		100.4152

				90.22		100.4152

				90.24		100.4152

				90.26		100.4152

				90.28		100.4152

				90.3		100.4152

				90.32		100.4152

				90.34		100.4152

				90.36		100.4152

				90.39		100.4152

				90.41		100.4152

				90.43		100.4152

				90.45		100.4152

				90.47		100.4152

				90.49		100.4152

				90.51		100.4152

				90.53		100.4152

				90.55		100.4152

				90.58		100.4152

				90.6		100.4152

				90.62		100.4152

				90.64		100.4152

				90.66		100.4152

				90.68		100.4152

				90.7		100.4152

				90.72		100.4152

				90.74		100.4152

				90.77		100.4152

				90.79		100.4152

				90.81		100.4152

				90.83		100.4152

				90.85		100.4152

				90.87		100.4152

				90.89		100.4152

				90.91		100.4152

				90.93		100.4152

				90.95		100.4152

				90.98		100.4152

				91		100.4152

				91.02		100.4152

				91.04		100.4152

				91.06		100.4152

				91.08		100.4152

				91.1		100.4152

				91.12		100.4152

				91.14		100.4152

				91.17		100.4152

				91.19		100.4152

				91.21		100.4113

				91.23		100.4113

				91.25		100.4113

				91.27		100.4113

				91.29		100.4113

				91.31		100.4113

				91.33		100.4113

				91.36		100.4113

				91.38		100.4113

				91.4		100.4113

				91.42		100.4113

				91.44		100.4113

				91.46		100.4113

				91.48		100.4113

				91.5		100.4113

				91.52		100.4113

				91.54		100.4113

				91.57		100.4113

				91.59		100.4113

				91.61		100.4113

				91.63		100.4113

				91.65		100.4113

				91.67		100.4113

				91.69		100.4113

				91.71		100.4113

				91.73		100.4113

				91.76		100.4113

				91.78		100.4113

				91.8		100.4113

				91.82		100.4113

				91.84		100.4113

				91.86		100.4113

				91.88		100.4113

				91.9		100.4113

				91.92		100.4113

				91.95		100.4113

				91.97		100.4113

				91.99		100.4113

				92.01		100.4113

				92.03		100.4152

				92.05		100.4113

				92.07		100.4152

				92.09		100.4113

				92.11		100.4113

				92.14		100.4152

				92.16		100.4152

				92.18		100.4113

				92.2		100.4152

				92.22		100.4113

				92.24		100.4113

				92.26		100.4113

				92.28		100.4152

				92.3		100.4152

				92.32		100.4152

				92.35		100.4152

				92.37		100.4152

				92.39		100.4152

				92.41		100.4152

				92.43		100.4152

				92.45		100.4152

				92.47		100.4152

				92.49		100.4152

				92.51		100.4152

				92.54		100.4152

				92.56		100.4152

				92.58		100.4152

				92.6		100.4152

				92.62		100.4152

				92.64		100.4152

				92.66		100.4152

				92.68		100.4152

				92.7		100.4152

				92.73		100.4152

				92.75		100.4152

				92.77		100.4152

				92.79		100.4152

				92.81		100.4152

				92.83		100.4113

				92.85		100.4152

				92.87		100.4152

				92.89		100.4152

				92.92		100.4152

				92.94		100.4152

				92.96		100.4152

				92.98		100.4152

				93		100.4152

				93.02		100.4152

				93.04		100.4152

				93.06		100.4152

				93.08		100.4152

				93.1		100.4152

				93.13		100.4152

				93.15		100.4152

				93.17		100.4152

				93.19		100.4152

				93.21		100.4152

				93.23		100.4152

				93.25		100.4152

				93.27		100.4152

				93.29		100.4152

				93.32		100.4152

				93.34		100.4152

				93.36		100.4152

				93.38		100.4152

				93.4		100.4152

				93.42		100.4152

				93.44		100.4152

				93.46		100.4152

				93.48		100.4152

				93.5		100.4152

				93.53		100.4152

				93.55		100.4152

				93.57		100.419

				93.59		100.4152

				93.61		100.4152

				93.63		100.4152

				93.65		100.4152

				93.67		100.4152

				93.69		100.4152

				93.72		100.4152

				93.74		100.4152

				93.76		100.4152

				93.78		100.4152

				93.8		100.4152

				93.82		100.4152

				93.84		100.4152

				93.86		100.419

				93.88		100.419

				93.91		100.419

				93.93		100.419

				93.95		100.419

				93.97		100.419

				93.99		100.419

				94.01		100.419

				94.03		100.419

				94.05		100.419

				94.07		100.419

				94.09		100.419

				94.12		100.419

				94.14		100.419

				94.16		100.419

				94.18		100.419

				94.2		100.419

				94.22		100.419

				94.24		100.419

				94.26		100.419

				94.28		100.419

				94.31		100.419

				94.33		100.419

				94.35		100.419

				94.37		100.419

				94.39		100.419

				94.41		100.419

				94.43		100.419

				94.45		100.419

				94.47		100.4229

				94.49		100.4229

				94.52		100.419

				94.54		100.419

				94.56		100.419

				94.58		100.419

				94.6		100.419

				94.62		100.419

				94.64		100.419

				94.66		100.419

				94.68		100.419

				94.7		100.419

				94.73		100.419

				94.75		100.419

				94.77		100.419

				94.79		100.419

				94.81		100.419

				94.83		100.419

				94.85		100.4229

				94.87		100.419

				94.89		100.4229

				94.92		100.419

				94.94		100.419

				94.96		100.419

				94.98		100.419

				95		100.419

				95.02		100.419

				95.04		100.419

				95.06		100.419

				95.08		100.419

				95.1		100.419

				95.13		100.419

				95.15		100.419

				95.17		100.419

				95.19		100.419

				95.21		100.419

				95.23		100.419

				95.25		100.419

				95.27		100.419

				95.29		100.4229

				95.32		100.4229

				95.34		100.419

				95.36		100.4229

				95.38		100.4229

				95.4		100.4229

				95.42		100.419

				95.44		100.4229

				95.46		100.4229

				95.48		100.4229

				95.5		100.419

				95.53		100.4229

				95.55		100.419

				95.57		100.419

				95.59		100.419

				95.61		100.419

				95.63		100.419

				95.65		100.419

				95.67		100.419

				95.69		100.419

				95.72		100.419

				95.74		100.419

				95.76		100.419

				95.78		100.419

				95.8		100.419

				95.82		100.419

				95.84		100.419

				95.86		100.419

				95.88		100.419

				95.9		100.419

				95.93		100.419

				95.95		100.419

				95.97		100.419

				95.99		100.419

				96.01		100.419

				96.03		100.4152

				96.05		100.419

				96.07		100.419

				96.09		100.4152

				96.12		100.4152

				96.14		100.4152

				96.16		100.4152

				96.18		100.4152

				96.2		100.4152

				96.22		100.4152

				96.24		100.4152

				96.26		100.4152

				96.28		100.4152

				96.3		100.4152

				96.33		100.4152

				96.35		100.4152

				96.37		100.4152

				96.39		100.4152

				96.41		100.4152

				96.43		100.4152

				96.45		100.4152

				96.47		100.4152

				96.49		100.4152

				96.52		100.4152

				96.54		100.4152

				96.56		100.4152

				96.58		100.4152

				96.6		100.4152

				96.62		100.4152

				96.64		100.4152

				96.66		100.4152

				96.68		100.4152

				96.7		100.4152

				96.73		100.4152

				96.75		100.4152

				96.77		100.4152

				96.79		100.4152

				96.81		100.4152

				96.83		100.4152

				96.85		100.4152

				96.87		100.4152

				96.89		100.4152

				96.92		100.4152

				96.94		100.4152

				96.96		100.4152

				96.98		100.4152

				97		100.4152

				97.02		100.4152

				97.04		100.4113

				97.06		100.4152

				97.08		100.4152

				97.1		100.4113

				97.13		100.4152

				97.15		100.4152

				97.17		100.4113

				97.19		100.4113

				97.21		100.4113

				97.23		100.4113

				97.25		100.4113

				97.27		100.4152

				97.29		100.4152

				97.32		100.4113

				97.34		100.4074

				97.36		100.4035

				97.38		100.4035

				97.4		100.3996

				97.42		100.3996

				97.44		100.4035

				97.46		100.3996

				97.48		100.3996

				97.5		100.3996

				97.53		100.3996

				97.55		100.3996

				97.57		100.3996

				97.59		100.3996

				97.61		100.3996

				97.63		100.3996

				97.65		100.3996

				97.67		100.3996

				97.69		100.3996

				97.72		100.3996

				97.74		100.3996

				97.76		100.3996

				97.78		100.4035

				97.8		100.4035

				97.82		100.4035

				97.84		100.4035

				97.86		100.4035

				97.88		100.4035

				97.91		100.4035

				97.93		100.4035

				97.95		100.4035

				97.97		100.4035

				97.99		100.4035

				98.01		100.4035

				98.03		100.4035

				98.05		100.4035

				98.07		100.4035

				98.09		100.4035

				98.12		100.4035

				98.14		100.4035

				98.16		100.4035

				98.18		100.4035

				98.2		100.4035

				98.22		100.4035

				98.24		100.4035

				98.26		100.4035

				98.28		100.4035

				98.31		100.4035

				98.33		100.4035

				98.35		100.4074

				98.37		100.4074

				98.39		100.4074

				98.41		100.4074

				98.43		100.4074

				98.45		100.4074

				98.47		100.4074

				98.49		100.4074

				98.52		100.4074

				98.54		100.4074

				98.56		100.4074

				98.58		100.4074

				98.6		100.4074

				98.62		100.4074

				98.64		100.4035

				98.66		100.4035

				98.68		100.4035

				98.7		100.4035

				98.73		100.4035

				98.75		100.4035

				98.77		100.4035

				98.79		100.4035

				98.81		100.4035

				98.83		100.4035

				98.85		100.4035

				98.87		100.3996

				98.89		100.4035

				98.91		100.419

				98.94		100.4229

				98.96		100.4229

				98.98		100.4268

				99		100.4268

				99.02		100.4268

				99.04		100.4268

				99.06		100.4307

				99.08		100.4346

				99.1		100.4423

				99.13		100.4462

				99.15		100.4578

				99.17		100.4656

				99.19		100.4695

				99.21		100.4695

				99.23		100.4695

				99.25		100.4734

				99.27		100.4695

				99.29		100.4695

				99.31		100.4695

				99.34		100.4656

				99.36		100.4656

				99.38		100.4656

				99.4		100.4656

				99.42		100.4656

				99.44		100.4617

				99.46		100.4578

				99.48		100.4578

				99.5		100.454

				99.52		100.454

				99.55		100.4501

				99.57		100.4501

				99.59		100.4462

				99.61		100.4462

				99.63		100.4501

				99.65		100.4501

				99.67		100.4501

				99.69		100.4501

				99.71		100.4501

				99.73		100.4501

				99.76		100.4501

				99.78		100.4501

				99.8		100.4501

				99.82		100.4501

				99.84		100.454

				99.86		100.4501

				99.88		100.4501

				99.9		100.4501

				99.92		100.4501

				99.95		100.4501

				99.97		100.4501

				99.99		100.4462

				100.01		100.4462

				100.03		100.4462

				100.05		100.4462

				100.07		100.4462

				100.09		100.4462

				100.11		100.4462

				100.13		100.4462

				100.16		100.4462

				100.18		100.4462

				100.2		100.4462

				100.22		100.4462

				100.24		100.4462

				100.26		100.4462

				100.28		100.4462

				100.3		100.4462

				100.32		100.4462

				100.35		100.4423

				100.37		100.4423

				100.39		100.4384

				100.41		100.4346

				100.43		100.4307

				100.45		100.4268

				100.47		100.4268

				100.49		100.4268

				100.51		100.4268

				100.53		100.4268

				100.56		100.4268

				100.58		100.4268

				100.6		100.4268

				100.62		100.4268

				100.64		100.4268

				100.66		100.4229

				100.68		100.4229

				100.7		100.4229

				100.72		100.4229

				100.74		100.4229

				100.77		100.4229

				100.79		100.4268

				100.81		100.4268

				100.83		100.4268

				100.85		100.4268

				100.87		100.4268

				100.89		100.4268

				100.91		100.4268

				100.93		100.4268

				100.95		100.4268

				100.98		100.4268

				101		100.4268

				101.02		100.4268

				101.04		100.4268

				101.06		100.4307

				101.08		100.4307

				101.1		100.4307

				101.12		100.4307

				101.14		100.4307

				101.17		100.4307

				101.19		100.4307

				101.21		100.4307

				101.23		100.4307

				101.25		100.4307

				101.27		100.4307

				101.29		100.4307

				101.31		100.4307

				101.33		100.4307

				101.35		100.4307

				101.38		100.4307

				101.4		100.4307

				101.42		100.4307

				101.44		100.4307

				101.46		100.4307

				101.48		100.4307

				101.5		100.4307

				101.52		100.4307

				101.54		100.4307

				101.56		100.4307

				101.59		100.4307

				101.61		100.4307

				101.63		100.4307

				101.65		100.4307

				101.67		100.4307

				101.69		100.4307

				101.71		100.4307

				101.73		100.4307

				101.75		100.4307

				101.78		100.4307

				101.8		100.4307

				101.82		100.4307

				101.84		100.4307

				101.86		100.4307

				101.88		100.4307

				101.9		100.4307

				101.92		100.4307

				101.94		100.4307

				101.96		100.4307

				101.99		100.4307

				102.01		100.4307

				102.03		100.4307

				102.05		100.4307

				102.07		100.4307

				102.09		100.4346

				102.11		100.4307

				102.13		100.4307

				102.15		100.4307

				102.17		100.4307

				102.2		100.4307

				102.22		100.4307

				102.24		100.4307

				102.26		100.4307

				102.28		100.4307

				102.3		100.4307

				102.32		100.4307

				102.34		100.4307

				102.36		100.4307

				102.38		100.4307

				102.41		100.4307

				102.43		100.4307

				102.45		100.4307

				102.47		100.4307

				102.49		100.4307

				102.51		100.4346

				102.53		100.4346

				102.55		100.4346

				102.57		100.4346

				102.59		100.4346

				102.62		100.4346

				102.64		100.4346

				102.66		100.4346

				102.68		100.4346

				102.7		100.4346

				102.72		100.4346

				102.74		100.4346

				102.76		100.4346

				102.78		100.4346

				102.81		100.4346

				102.83		100.4346

				102.85		100.4346

				102.87		100.4346

				102.89		100.4346

				102.91		100.4346

				102.93		100.4346

				102.95		100.4346

				102.97		100.4307

				102.99		100.4346

				103.02		100.4346

				103.04		100.4307

				103.06		100.4346

				103.08		100.4307

				103.1		100.4346

				103.12		100.4307

				103.14		100.4307

				103.16		100.4307

				103.18		100.4346

				103.2		100.4307

				103.23		100.4346

				103.25		100.4346

				103.27		100.4307

				103.29		100.4346

				103.31		100.4346

				103.33		100.4346

				103.35		100.4307

				103.37		100.4346

				103.39		100.4346

				103.41		100.4346

				103.44		100.4346

				103.46		100.4346

				103.48		100.4346

				103.5		100.4346

				103.52		100.4346

				103.54		100.4346

				103.56		100.4346

				103.58		100.4346

				103.6		100.4346

				103.63		100.4307

				103.65		100.4307

				103.67		100.4346

				103.69		100.4346

				103.71		100.4346

				103.73		100.4346

				103.75		100.4346

				103.77		100.4346

				103.79		100.4346

				103.81		100.4346

				103.84		100.4346

				103.86		100.4346

				103.88		100.4346

				103.9		100.4346

				103.92		100.4346

				103.94		100.4346

				103.96		100.4346

				103.98		100.4346

				104		100.4346

				104.02		100.4346

				104.05		100.4346

				104.07		100.4346

				104.09		100.4346

				104.11		100.4346

				104.13		100.4346

				104.15		100.4346

				104.17		100.4346

				104.19		100.4346

				104.21		100.4346

				104.23		100.4346

				104.26		100.4346

				104.28		100.4346

				104.3		100.4346

				104.32		100.4346

				104.34		100.4346

				104.36		100.4346

				104.38		100.4346

				104.4		100.4346

				104.42		100.4346

				104.44		100.4346

				104.47		100.4346

				104.49		100.4346

				104.51		100.4346

				104.53		100.4346

				104.55		100.4346

				104.57		100.4346

				104.59		100.4346

				104.61		100.4346

				104.63		100.4346

				104.66		100.4346

				104.68		100.4346

				104.7		100.4346

				104.72		100.4346

				104.74		100.4346

				104.76		100.4346

				104.78		100.4346

				104.8		100.4346

				104.82		100.4346

				104.84		100.4346

				104.87		100.4346

				104.89		100.4384

				104.91		100.4384

				104.93		100.4384

				104.95		100.4384

				104.97		100.4384

				104.99		100.4384

				105.01		100.4384

				105.03		100.4384

				105.05		100.4384

				105.08		100.4384

				105.1		100.4384

				105.12		100.4384

				105.14		100.4346

				105.16		100.4384

				105.18		100.4346

				105.2		100.4384

				105.22		100.4384

				105.24		100.4384

				105.26		100.4384

				105.29		100.4346

				105.31		100.4384

				105.33		100.4346

				105.35		100.4384

				105.37		100.4346

				105.39		100.4346

				105.41		100.4346

				105.43		100.4346

				105.45		100.4346

				105.47		100.4346

				105.5		100.4346

				105.52		100.4346

				105.54		100.4346

				105.56		100.4346

				105.58		100.4346

				105.6		100.4346

				105.62		100.4346

				105.64		100.4346

				105.66		100.4346

				105.69		100.4346

				105.71		100.4346

				105.73		100.4346

				105.75		100.4346

				105.77		100.4346

				105.79		100.4346

				105.81		100.4346

				105.83		100.4346

				105.85		100.4346

				105.87		100.4346

				105.9		100.4346

				105.92		100.4346

				105.94		100.4346

				105.96		100.4346

				105.98		100.4346

				106		100.4346

				106.02		100.4346

				106.04		100.4346

				106.06		100.4346

				106.08		100.4346

				106.11		100.4346

				106.13		100.4346

				106.15		100.4346

				106.17		100.4346

				106.19		100.4346

				106.21		100.4346

				106.23		100.4346

				106.25		100.4346

				106.27		100.4346

				106.29		100.4346

				106.32		100.4346

				106.34		100.4346

				106.36		100.4346

				106.38		100.4346

				106.4		100.4346

				106.42		100.4346

				106.44		100.4346

				106.46		100.4346

				106.48		100.4346

				106.51		100.4346

				106.53		100.4346

				106.55		100.4346

				106.57		100.4346

				106.59		100.4346

				106.61		100.4346

				106.63		100.4346

				106.65		100.4307

				106.67		100.4307

				106.69		100.4307

				106.72		100.4307

				106.74		100.4307

				106.76		100.4307

				106.78		100.4307

				106.8		100.4307

				106.82		100.4307

				106.84		100.4307

				106.86		100.4307

				106.88		100.4307

				106.9		100.4307

				106.93		100.4307

				106.95		100.4307

				106.97		100.4307

				106.99		100.4307

				107.01		100.4307

				107.03		100.4307

				107.05		100.4307

				107.07		100.4307

				107.09		100.4307

				107.12		100.4307

				107.14		100.4307

				107.16		100.4307

				107.18		100.4307

				107.2		100.4307

				107.22		100.4307

				107.24		100.4307

				107.26		100.4307

				107.28		100.4307

				107.3		100.4307

				107.33		100.4307

				107.35		100.4307

				107.37		100.4307

				107.39		100.4307

				107.41		100.4307

				107.43		100.4307

				107.45		100.4307

				107.47		100.4346

				107.49		100.4346

				107.51		100.4346

				107.54		100.4346

				107.56		100.4346

				107.58		100.4346

				107.6		100.4346

				107.62		100.4346

				107.64		100.4346

				107.66		100.4346

				107.68		100.4346

				107.7		100.4346

				107.72		100.4346

				107.75		100.4346

				107.77		100.4346

				107.79		100.4346

				107.81		100.4346

				107.83		100.4346

				107.85		100.4346

				107.87		100.4346

				107.89		100.4346

				107.91		100.4384

				107.94		100.4384

				107.96		100.4384

				107.98		100.4384

				108		100.4384

				108.02		100.4384

				108.04		100.4384

				108.06		100.4384

				108.08		100.4384

				108.1		100.4384

				108.12		100.4384

				108.15		100.4384

				108.17		100.4384

				108.19		100.4384

				108.21		100.4384

				108.23		100.4384

				108.25		100.4384

				108.27		100.4384

				108.29		100.4384

				108.31		100.4384

				108.33		100.4384

				108.36		100.4423

				108.38		100.4384

				108.4		100.4384

				108.42		100.4384

				108.44		100.4384

				108.46		100.4423

				108.48		100.4384

				108.5		100.4423

				108.52		100.4423

				108.55		100.4423

				108.57		100.4423

				108.59		100.4423

				108.61		100.4423

				108.63		100.4423

				108.65		100.4423

				108.67		100.4423

				108.69		100.4423

				108.71		100.4423

				108.73		100.4423

				108.76		100.4423

				108.78		100.4423

				108.8		100.4423

				108.82		100.4423

				108.84		100.4423

				108.86		100.4423

				108.88		100.4423

				108.9		100.4423

				108.92		100.4423

				108.94		100.4462

				108.97		100.4423

				108.99		100.4423

				109.01		100.4462

				109.03		100.4423

				109.05		100.4462

				109.07		100.4462

				109.09		100.4462

				109.11		100.4462

				109.13		100.4462

				109.15		100.4462

				109.18		100.4462

				109.2		100.4462

				109.22		100.4462

				109.24		100.4462

				109.26		100.4462

				109.28		100.4462

				109.3		100.4462

				109.32		100.4462

				109.34		100.4462

				109.37		100.4462

				109.39		100.4462

				109.41		100.4462

				109.43		100.4462

				109.45		100.4462

				109.47		100.4462

				109.49		100.4462

				109.51		100.4462

				109.53		100.4462

				109.55		100.4462

				109.58		100.4462

				109.6		100.4423

				109.62		100.4423

				109.64		100.4423

				109.66		100.4462

				109.68		100.4423

				109.7		100.4423

				109.72		100.4423

				109.74		100.4423

				109.76		100.4423

				109.79		100.4423

				109.81		100.4423

				109.83		100.4423

				109.85		100.4423

				109.87		100.4423

				109.89		100.4423

				109.91		100.4423

				109.93		100.4423

				109.95		100.4423

				109.97		100.4423

				110		100.4423

				110.02		100.4423

				110.04		100.4423

				110.06		100.4423

				110.08		100.4423

				110.1		100.4423

				110.12		100.4423

				110.14		100.4423

				110.16		100.4423

				110.19		100.4423

				110.21		100.4423

				110.23		100.4423

				110.25		100.4423

				110.27		100.4423

				110.29		100.4423

				110.31		100.4423

				110.33		100.4423

				110.35		100.4423

				110.37		100.4423

				110.4		100.4423

				110.42		100.4423

				110.44		100.4423

				110.46		100.4423

				110.48		100.4423

				110.5		100.4423

				110.52		100.4423

				110.54		100.4423

				110.56		100.4423

				110.58		100.4423

				110.61		100.4423

				110.63		100.4423

				110.65		100.4423

				110.67		100.4423

				110.69		100.4423

				110.71		100.4423

				110.73		100.4423

				110.75		100.4423

				110.77		100.4423

				110.79		100.4423

				110.82		100.4423

				110.84		100.4423

				110.86		100.4423

				110.88		100.4423

				110.9		100.4423

				110.92		100.4423

				110.94		100.4423

				110.96		100.4423

				110.98		100.4423

				111		100.4423

				111.03		100.4423

				111.05		100.4462

				111.07		100.4423

				111.09		100.4423

				111.11		100.4423

				111.13		100.4423

				111.15		100.4423

				111.17		100.4423

				111.19		100.4423

				111.22		100.4423

				111.24		100.4423

				111.26		100.4423

				111.28		100.4423

				111.3		100.4423

				111.32		100.4423

				111.34		100.4423

				111.36		100.4423

				111.38		100.4423

				111.4		100.4423

				111.43		100.4462

				111.45		100.4462

				111.47		100.4462

				111.49		100.4462

				111.51		100.4462

				111.53		100.4462

				111.55		100.4462

				111.57		100.4462

				111.59		100.4462

				111.61		100.4462

				111.64		100.4462

				111.66		100.4462

				111.68		100.4462

				111.7		100.4462

				111.72		100.4462

				111.74		100.4462

				111.76		100.4462

				111.78		100.4462

				111.8		100.4462

				111.83		100.4462

				111.85		100.4462

				111.87		100.4462

				111.89		100.4462

				111.91		100.4462

				111.93		100.4462

				111.95		100.4462

				111.97		100.4462

				111.99		100.4462

				112.01		100.4462

				112.04		100.4462

				112.06		100.4462

				112.08		100.4462

				112.1		100.4462

				112.12		100.4462

				112.14		100.4462

				112.16		100.4462

				112.18		100.4462

				112.2		100.4462

				112.22		100.4462

				112.25		100.4462

				112.27		100.4462

				112.29		100.4462

				112.31		100.4462

				112.33		100.4462

				112.35		100.4462

				112.37		100.4501

				112.39		100.4501

				112.41		100.4501

				112.43		100.4501

				112.46		100.4501

				112.48		100.4501

				112.5		100.4501

				112.52		100.4501

				112.54		100.4501

				112.56		100.4501

				112.58		100.4501

				112.6		100.4501

				112.62		100.4501

				112.64		100.4462

				112.67		100.4501

				112.69		100.4501

				112.71		100.4501

				112.73		100.4462

				112.75		100.4462

				112.77		100.4462

				112.79		100.4462

				112.81		100.4462

				112.83		100.4462

				112.86		100.4501

				112.88		100.4501

				112.9		100.4462

				112.92		100.4501

				112.94		100.4501

				112.96		100.4501

				112.98		100.4501

				113		100.4501

				113.02		100.4501

				113.04		100.4501

				113.07		100.4462

				113.09		100.4462

				113.11		100.4462

				113.13		100.4462

				113.15		100.4462

				113.17		100.4462

				113.19		100.4462

				113.21		100.4462

				113.23		100.4462

				113.25		100.4462

				113.28		100.4462

				113.3		100.4462

				113.32		100.4462

				113.34		100.4462

				113.36		100.4462

				113.38		100.4462

				113.4		100.4462

				113.42		100.4462

				113.44		100.4501

				113.46		100.4462

				113.49		100.4462

				113.51		100.4462

				113.53		100.4462

				113.55		100.4462

				113.57		100.4462

				113.59		100.4462

				113.61		100.4462

				113.63		100.4462

				113.65		100.4462

				113.67		100.4462

				113.7		100.4462

				113.72		100.4462

				113.74		100.4462

				113.76		100.4462

				113.78		100.4462

				113.8		100.4462

				113.82		100.4462

				113.84		100.4462

				113.86		100.4462

				113.88		100.4462

				113.91		100.4462

				113.93		100.4462

				113.95		100.4462

				113.97		100.4462

				113.99		100.4462

				114.01		100.4462

				114.03		100.4462

				114.05		100.4462

				114.07		100.4462

				114.09		100.4423

				114.12		100.4423

				114.14		100.4462

				114.16		100.4423

				114.18		100.4423

				114.2		100.4423

				114.22		100.4423

				114.24		100.4423

				114.26		100.4423

				114.28		100.4423

				114.31		100.4423

				114.33		100.4423

				114.35		100.4423

				114.37		100.4423

				114.39		100.4423

				114.41		100.4423

				114.43		100.4423

				114.45		100.4423

				114.47		100.4384

				114.49		100.4423

				114.52		100.4423

				114.54		100.4384

				114.56		100.4384

				114.58		100.4384

				114.6		100.4384

				114.62		100.4384

				114.64		100.4384

				114.66		100.4384

				114.68		100.4384

				114.7		100.4423

				114.73		100.4384

				114.75		100.4423

				114.77		100.4423

				114.79		100.4423

				114.81		100.4423

				114.83		100.4423

				114.85		100.4423

				114.87		100.4423

				114.89		100.4423

				114.91		100.4423

				114.94		100.4423

				114.96		100.4423

				114.98		100.4423

				115		100.4384

				115.02		100.4384

				115.04		100.4384

				115.06		100.4384

				115.08		100.4384

				115.1		100.4384

				115.13		100.4384

				115.15		100.4384

				115.17		100.4384

				115.19		100.4384

				115.21		100.4384

				115.23		100.4384

				115.25		100.4384

				115.27		100.4384

				115.29		100.4384

				115.31		100.4384

				115.34		100.4384

				115.36		100.4384

				115.38		100.4384

				115.4		100.4384

				115.42		100.4384

				115.44		100.4384

				115.46		100.4384

				115.48		100.4384

				115.5		100.4384

				115.52		100.4346

				115.55		100.4346

				115.57		100.4346

				115.59		100.4346

				115.61		100.4346

				115.63		100.4346

				115.65		100.4346

				115.67		100.4346

				115.69		100.4384

				115.71		100.4384

				115.74		100.4384

				115.76		100.4384

				115.78		100.4384

				115.8		100.4384

				115.82		100.4346

				115.84		100.4384

				115.86		100.4384

				115.88		100.4346

				115.9		100.4384

				115.92		100.4346

				115.95		100.4346

				115.97		100.4346

				115.99		100.4346

				116.01		100.4346

				116.03		100.4346

				116.05		100.4346

				116.07		100.4346

				116.09		100.4346

				116.11		100.4346

				116.13		100.4346

				116.16		100.4346

				116.18		100.4346

				116.2		100.4346

				116.22		100.4346

				116.24		100.4346

				116.26		100.4346

				116.28		100.4346

				116.3		100.4346

				116.32		100.4346

				116.34		100.4346

				116.37		100.4346

				116.39		100.4346

				116.41		100.4346

				116.43		100.4346

				116.45		100.4346

				116.47		100.4346

				116.49		100.4346

				116.51		100.4346

				116.53		100.4346

				116.55		100.4346

				116.58		100.4346

				116.6		100.4346

				116.62		100.4346

				116.64		100.4346

				116.66		100.4346

				116.68		100.4346

				116.7		100.4346

				116.72		100.4346

				116.74		100.4346

				116.76		100.4346

				116.79		100.4346

				116.81		100.4346

				116.83		100.4346

				116.85		100.4346

				116.87		100.4346

				116.89		100.4346

				116.91		100.4346

				116.93		100.4346

				116.95		100.4346

				116.98		100.4346

				117		100.4346

				117.02		100.4346

				117.04		100.4346

				117.06		100.4346

				117.08		100.4346

				117.1		100.4346

				117.12		100.4346

				117.14		100.4346

				117.16		100.4346

				117.19		100.4346

				117.21		100.4346

				117.23		100.4346

				117.25		100.4346

				117.27		100.4346

				117.29		100.4384

				117.31		100.4384

				117.33		100.4384

				117.35		100.4384

				117.38		100.4346

				117.4		100.4346

				117.42		100.4346

				117.44		100.4346

				117.46		100.4346

				117.48		100.4346

				117.5		100.4346

				117.52		100.4346

				117.54		100.4346

				117.56		100.4346

				117.59		100.4346

				117.61		100.4346

				117.63		100.4346

				117.65		100.4346

				117.67		100.4346

				117.69		100.4384

				117.71		100.4346

				117.73		100.4346

				117.75		100.4346

				117.77		100.4346

				117.8		100.4346

				117.82		100.4346

				117.84		100.4346

				117.86		100.4346

				117.88		100.4346

				117.9		100.4346

				117.92		100.4346

				117.94		100.4346

				117.96		100.4346

				117.99		100.4346

				118.01		100.4346

				118.03		100.4346

				118.05		100.4346

				118.07		100.4346

				118.09		100.4346

				118.11		100.4346

				118.13		100.4346

				118.15		100.4346

				118.17		100.4346

				118.2		100.4346

				118.22		100.4346

				118.24		100.4346

				118.26		100.4346

				118.28		100.4346

				118.3		100.4346

				118.32		100.4346

				118.34		100.4346

				118.36		100.4346

				118.38		100.4346

				118.41		100.4346

				118.43		100.4346

				118.45		100.4346

				118.47		100.4346

				118.49		100.4346

				118.51		100.4346

				118.53		100.4346

				118.55		100.4346

				118.57		100.4346

				118.6		100.4346

				118.62		100.4346

				118.64		100.4346

				118.66		100.4346

				118.68		100.4346

				118.7		100.4346

				118.72		100.4346

				118.74		100.4346

				118.76		100.4346

				118.78		100.4346

				118.81		100.4346

				118.83		100.4346

				118.85		100.4346

				118.87		100.4346

				118.89		100.4346

				118.91		100.4346

				118.93		100.4346

				118.95		100.4346

				118.97		100.4346

				118.99		100.4346

				119.02		100.4346

				119.04		100.4346

				119.06		100.4346

				119.08		100.4346

				119.1		100.4346

				119.12		100.4346

				119.14		100.4346

				119.16		100.4346

				119.18		100.4346

				119.21		100.4346

				119.23		100.4346

				119.25		100.4346

				119.27		100.4346

				119.29		100.4346

				119.31		100.4346

				119.33		100.4346

				119.35		100.4346

				119.37		100.4346

				119.39		100.4307

				119.42		100.4346

				119.44		100.4346

				119.46		100.4346

				119.48		100.4346

				119.5		100.4346

				119.52		100.4346

				119.54		100.4346

				119.56		100.4346

				119.58		100.4346

				119.6		100.4346

				119.63		100.4346

				119.65		100.4384

				119.67		100.4346

				119.69		100.4346

				119.71		100.4346

				119.73		100.4346

				119.75		100.4346

				119.77		100.4346

				119.79		100.4346

				119.81		100.4346

				119.84		100.4346

				119.86		100.4346

				119.88		100.4346

				119.9		100.4346

				119.92		100.4346

				119.94		100.4346

				119.96		100.4346

				119.98		100.4346

				120		100.4346

				120.03		100.4346

				120.05		100.4307

				120.07		100.4346

				120.09		100.4384

				120.11		100.4384

				120.13		100.4346

				120.15		100.4384

				120.17		100.4346

				120.19		100.4346

				120.21		100.4346

				120.24		100.4346

				120.26		100.4346

				120.28		100.4346

				120.3		100.4346

				120.32		100.4346

				120.34		100.4346

				120.36		100.4346

				120.38		100.4346

				120.4		100.4346

				120.42		100.4346

				120.45		100.4346

				120.47		100.4346

				120.49		100.4346

				120.51		100.4346

				120.53		100.4346

				120.55		100.4346

				120.57		100.4346

				120.59		100.4346

				120.61		100.4346

				120.63		100.4346

				120.66		100.4346

				120.68		100.4346

				120.7		100.4346

				120.72		100.4346

				120.74		100.4346

				120.76		100.4346

				120.78		100.4346

				120.8		100.4346

				120.82		100.4346

				120.85		100.4346

				120.87		100.4346

				120.89		100.4346

				120.91		100.4346

				120.93		100.4346

				120.95		100.4346

				120.97		100.4346

				120.99		100.4346

				121.01		100.4346

				121.03		100.4346

				121.06		100.4346

				121.08		100.4346

				121.1		100.4346

				121.12		100.4346

				121.14		100.4346

				121.16		100.4346

				121.18		100.4346

				121.2		100.4346

				121.22		100.4346

				121.25		100.4346

				121.27		100.4346

				121.29		100.4346

				121.31		100.4307

				121.33		100.4307

				121.35		100.4307

				121.37		100.4346

				121.39		100.4346

				121.41		100.4346

				121.43		100.4346

				121.46		100.4307

				121.48		100.4346

				121.5		100.4346

				121.52		100.4346

				121.54		100.4346

				121.56		100.4346

				121.58		100.4346

				121.6		100.4346

				121.62		100.4307

				121.65		100.4307

				121.67		100.4307

				121.69		100.4307

				121.71		100.4307

				121.73		100.4268

				121.75		100.4268

				121.77		100.4268

				121.79		100.4268

				121.81		100.4268

				121.83		100.4268

				121.86		100.4268

				121.88		100.4268

				121.9		100.4268

				121.92		100.4268

				121.94		100.4268

				121.96		100.4268

				121.98		100.4268

				122		100.4268

				122.02		100.4268

				122.05		100.4268

				122.07		100.4268

				122.09		100.4268

				122.11		100.4268

				122.13		100.4307

				122.15		100.4268

				122.17		100.4229

				122.19		100.4229

				122.21		100.4229

				122.23		100.4229

				122.26		100.4229

				122.28		100.4229

				122.3		100.4229

				122.32		100.4229

				122.34		100.4229

				122.36		100.4229

				122.38		100.4229

				122.4		100.4229

				122.42		100.4229

				122.45		100.4229

				122.47		100.4229

				122.49		100.4229

				122.51		100.4229

				122.53		100.4229

				122.55		100.419

				122.57		100.4229

				122.59		100.4229

				122.61		100.4229

				122.63		100.419

				122.66		100.419

				122.68		100.419

				122.7		100.419

				122.72		100.419

				122.74		100.419

				122.76		100.419

				122.78		100.419

				122.8		100.419

				122.82		100.419

				122.84		100.419

				122.87		100.419

				122.89		100.419

				122.91		100.419

				122.93		100.419

				122.95		100.419

				122.97		100.419

				122.99		100.419

				123.01		100.4152

				123.03		100.4152

				123.06		100.4152

				123.08		100.4152

				123.1		100.4152

				123.12		100.4152

				123.14		100.4152

				123.16		100.4152

				123.18		100.4152

				123.2		100.4152

				123.22		100.4152

				123.24		100.4152

				123.27		100.4152

				123.29		100.4152

				123.31		100.4152

				123.33		100.4152

				123.35		100.4152

				123.37		100.4152

				123.39		100.4152

				123.41		100.4152

				123.43		100.4152

				123.46		100.4152

				123.48		100.4152

				123.5		100.4113

				123.52		100.4152

				123.54		100.4152

				123.56		100.4113

				123.58		100.4113

				123.6		100.4113

				123.62		100.4113

				123.64		100.4113

				123.67		100.4113

				123.69		100.4113

				123.71		100.4113

				123.73		100.4113

				123.75		100.4113

				123.77		100.4113

				123.79		100.4113

				123.81		100.4113

				123.83		100.4113

				123.86		100.4113

				123.88		100.4113

				123.9		100.4113

				123.92		100.4113

				123.94		100.4113

				123.96		100.4113

				123.98		100.4113

				124		100.4113

				124.02		100.4113

				124.05		100.4113

				124.07		100.4113

				124.09		100.4113

				124.11		100.4113

				124.13		100.4113

				124.15		100.4113

				124.17		100.4113

				124.19		100.4113

				124.21		100.4113

				124.23		100.4113

				124.26		100.4113

				124.28		100.4113

				124.3		100.4113

				124.32		100.4113

				124.34		100.4113

				124.36		100.4113

				124.38		100.4113

				124.4		100.4113

				124.42		100.4113

				124.45		100.4113

				124.47		100.4113

				124.49		100.4113

				124.51		100.4113

				124.53		100.4113

				124.55		100.4113

				124.57		100.4113

				124.59		100.4113

				124.61		100.4113

				124.63		100.4113

				124.66		100.4113

				124.68		100.4113

				124.7		100.4113

				124.72		100.4113

				124.74		100.4113

				124.76		100.4074

				124.78		100.4113

				124.8		100.4113

				124.82		100.4113

				124.85		100.4113

				124.87		100.4113

				124.89		100.4074

				124.91		100.4074

				124.93		100.4113

				124.95		100.4113

				124.97		100.4113

				124.99		100.4113

				125.01		100.4113

				125.04		100.4113

				125.06		100.4113

				125.08		100.4113

				125.1		100.4113

				125.12		100.4113

				125.14		100.4113

				125.16		100.4113

				125.18		100.4074

				125.2		100.4074

				125.23		100.4074

				125.25		100.4074

				125.27		100.4074

				125.29		100.4074

				125.31		100.4074

				125.33		100.4074

				125.35		100.4074

				125.37		100.4074

				125.39		100.4074

				125.42		100.4074

				125.44		100.4074

				125.46		100.4074

				125.48		100.4074

				125.5		100.4074

				125.52		100.4074

				125.54		100.4074

				125.56		100.4074

				125.58		100.4074

				125.6		100.4074

				125.63		100.4074

				125.65		100.4074

				125.67		100.4074

				125.69		100.4035

				125.71		100.4074

				125.73		100.4074

				125.75		100.4074

				125.77		100.4074

				125.79		100.4035

				125.82		100.4035

				125.84		100.4035

				125.86		100.4035

				125.88		100.4035

				125.9		100.4074

				125.92		100.4074

				125.94		100.4035

				125.96		100.4035

				125.98		100.4035

				126.01		100.4074

				126.03		100.4035

				126.05		100.4074

				126.07		100.4074

				126.09		100.4035

				126.11		100.4035

				126.13		100.4035

				126.15		100.4035

				126.17		100.4035

				126.2		100.4035

				126.22		100.4035

				126.24		100.4035

				126.26		100.4035

				126.28		100.4035

				126.3		100.4035

				126.32		100.4035

				126.34		100.4035

				126.36		100.4035

				126.39		100.4035

				126.41		100.4035

				126.43		100.4035

				126.45		100.4035

				126.47		100.4035

				126.49		100.4035

				126.51		100.4035

				126.53		100.4035

				126.55		100.4035

				126.57		100.4035

				126.6		100.3996

				126.62		100.3996

				126.64		100.3996

				126.66		100.3996

				126.68		100.3996

				126.7		100.3996

				126.72		100.3996

				126.74		100.3996

				126.76		100.3996

				126.79		100.3996

				126.81		100.3996

				126.83		100.3996

				126.85		100.3996

				126.87		100.3996

				126.89		100.3996

				126.91		100.3996

				126.93		100.3996

				126.95		100.3996

				126.98		100.3996

				127		100.3996

				127.02		100.3996

				127.04		100.3996

				127.06		100.3996

				127.08		100.3996

				127.1		100.3996

				127.12		100.3996

				127.14		100.3996

				127.16		100.3996

				127.19		100.3996

				127.21		100.3996

				127.23		100.3996

				127.25		100.3996

				127.27		100.3996

				127.29		100.3996

				127.31		100.4035

				127.33		100.3996

				127.35		100.4035

				127.38		100.3996

				127.4		100.3996

				127.42		100.3996

				127.44		100.3996

				127.46		100.3996

				127.48		100.3996

				127.5		100.4035

				127.52		100.4035

				127.54		100.4035

				127.57		100.4035

				127.59		100.4035

				127.61		100.4035

				127.63		100.3996

				127.65		100.4035

				127.67		100.3996

				127.69		100.3996

				127.71		100.3996

				127.73		100.3996

				127.76		100.3996

				127.78		100.3996

				127.8		100.3996

				127.82		100.3996

				127.84		100.3996

				127.86		100.3996

				127.88		100.3996

				127.9		100.3996

				127.92		100.3996

				127.95		100.3996

				127.97		100.3996

				127.99		100.3996

				128.01		100.3996

				128.03		100.3996

				128.05		100.3996

				128.07		100.3996

				128.09		100.3996

				128.11		100.4035

				128.13		100.3996

				128.16		100.3996

				128.18		100.3996

				128.2		100.3996

				128.22		100.3996

				128.24		100.4035

				128.26		100.4035

				128.28		100.4035

				128.3		100.4035

				128.32		100.4035

				128.35		100.4035

				128.37		100.4035

				128.39		100.4035

				128.41		100.4035

				128.43		100.4035

				128.45		100.4035

				128.47		100.4035

				128.49		100.4035

				128.51		100.4035

				128.54		100.4035

				128.56		100.3996

				128.58		100.3996

				128.6		100.3996

				128.62		100.3996

				128.64		100.4035

				128.66		100.3996

				128.68		100.4035

				128.7		100.4035

				128.73		100.4035

				128.75		100.4035

				128.77		100.4035

				128.79		100.4035

				128.81		100.4035

				128.83		100.4035

				128.85		100.4035

				128.87		100.4035

				128.89		100.4035

				128.92		100.4035

				128.94		100.4035

				128.96		100.4035

				128.98		100.4035

				129		100.4035

				129.02		100.4035

				129.04		100.4035

				129.06		100.4035

				129.08		100.4035

				129.1		100.4035

				129.13		100.3996

				129.15		100.4035

				129.17		100.3996

				129.19		100.3996

				129.21		100.3996

				129.23		100.3996

				129.25		100.3996

				129.27		100.3996

				129.29		100.3996

				129.32		100.3996

				129.34		100.3996

				129.36		100.3996

				129.38		100.3996

				129.4		100.3996

				129.42		100.3996

				129.44		100.3996

				129.46		100.3996

				129.48		100.3996

				129.51		100.3996

				129.53		100.3996

				129.55		100.3996

				129.57		100.3996

				129.59		100.3996

				129.61		100.3996

				129.63		100.3996

				129.65		100.3996

				129.67		100.3996

				129.7		100.3996

				129.72		100.3996

				129.74		100.3996

				129.76		100.3996

				129.78		100.3996

				129.8		100.3996

				129.82		100.3996

				129.84		100.3996

				129.87		100.3996

				129.89		100.3958

				129.91		100.3996

				129.93		100.3996

				129.95		100.3996

				129.97		100.3996

				129.99		100.3996

				130.01		100.3996

				130.03		100.3996

				130.06		100.3996

				130.08		100.3996

				130.1		100.3996

				130.12		100.3996

				130.14		100.3996

				130.16		100.3996

				130.18		100.3958

				130.2		100.3958

				130.22		100.3958

				130.25		100.3958

				130.27		100.3958

				130.29		100.3958

				130.31		100.3958

				130.33		100.3958

				130.35		100.3958

				130.37		100.3958

				130.39		100.3958

				130.41		100.3958

				130.44		100.3958

				130.46		100.3958

				130.48		100.3958

				130.5		100.3958

				130.52		100.3958

				130.54		100.3958

				130.56		100.3958

				130.58		100.3958

				130.6		100.3958

				130.63		100.3958

				130.65		100.3958

				130.67		100.3958

				130.69		100.3919

				130.71		100.3958

				130.73		100.3919

				130.75		100.3958

				130.77		100.3919

				130.8		100.3919

				130.82		100.3919

				130.84		100.3919

				130.86		100.3919

				130.88		100.3919

				130.9		100.3919

				130.92		100.3919

				130.94		100.3919

				130.96		100.3919

				130.99		100.3919

				131.01		100.3919

				131.03		100.3919

				131.05		100.3919

				131.07		100.3919

				131.09		100.3919

				131.11		100.388

				131.13		100.388

				131.15		100.388

				131.18		100.388

				131.2		100.388

				131.22		100.388

				131.24		100.388

				131.26		100.388

				131.28		100.388

				131.3		100.388

				131.32		100.388

				131.34		100.388

				131.37		100.388

				131.39		100.388

				131.41		100.388

				131.43		100.388

				131.45		100.388

				131.47		100.3841

				131.49		100.3841

				131.51		100.3841

				131.53		100.3841

				131.56		100.3841

				131.58		100.3841

				131.6		100.3841

				131.62		100.3841

				131.64		100.3841

				131.66		100.3841

				131.68		100.3841

				131.7		100.3841

				131.72		100.3841

				131.75		100.3841

				131.77		100.3841

				131.79		100.3841

				131.81		100.3841

				131.83		100.3841

				131.85		100.3841

				131.87		100.3841

				131.89		100.3802

				131.91		100.3802

				131.94		100.3802

				131.96		100.3802

				131.98		100.3802

				132		100.3802

				132.02		100.3802

				132.04		100.3802

				132.06		100.3802

				132.08		100.3802

				132.11		100.3802

				132.13		100.3802

				132.15		100.3802

				132.17		100.3802

				132.19		100.3802

				132.21		100.3802

				132.23		100.3802

				132.25		100.3802

				132.27		100.3802

				132.3		100.3802

				132.32		100.3764

				132.34		100.3764

				132.36		100.3802

				132.38		100.3764

				132.4		100.3802

				132.42		100.3802

				132.44		100.3802

				132.46		100.3764

				132.49		100.3764

				132.51		100.3764

				132.53		100.3764

				132.55		100.3764

				132.57		100.3764

				132.59		100.3764

				132.61		100.3764

				132.63		100.3764

				132.65		100.3764

				132.68		100.3764

				132.7		100.3764

				132.72		100.3764

				132.74		100.3764

				132.76		100.3764

				132.78		100.3764

				132.8		100.3764

				132.82		100.3764

				132.85		100.3764

				132.87		100.3764

				132.89		100.3764

				132.91		100.3764

				132.93		100.3725

				132.95		100.3764

				132.97		100.3725

				132.99		100.3725

				133.01		100.3725

				133.04		100.3725

				133.06		100.3725

				133.08		100.3725

				133.1		100.3725

				133.12		100.3725

				133.14		100.3725

				133.16		100.3725

				133.18		100.3725

				133.2		100.3725

				133.23		100.3764

				133.25		100.3725

				133.27		100.3725

				133.29		100.3725

				133.31		100.3725

				133.33		100.3725

				133.35		100.3725

				133.37		100.3725

				133.4		100.3725

				133.42		100.3725

				133.44		100.3725

				133.46		100.3725

				133.48		100.3725

				133.5		100.3725

				133.52		100.3725

				133.54		100.3725

				133.56		100.3725

				133.59		100.3725

				133.61		100.3725

				133.63		100.3725

				133.65		100.3725

				133.67		100.3725

				133.69		100.3725

				133.71		100.3725

				133.73		100.3725

				133.75		100.3725

				133.78		100.3725

				133.8		100.3725

				133.82		100.3725

				133.84		100.3725

				133.86		100.3725

				133.88		100.3725

				133.9		100.3725

				133.92		100.3725

				133.95		100.3725

				133.97		100.3725

				133.99		100.3725

				134.01		100.3725

				134.03		100.3725

				134.05		100.3725

				134.07		100.3725

				134.09		100.3725

				134.11		100.3725

				134.14		100.3725

				134.16		100.3725

				134.18		100.3725

				134.2		100.3725

				134.22		100.3686

				134.24		100.3725

				134.26		100.3725

				134.28		100.3686

				134.3		100.3725

				134.33		100.3725

				134.35		100.3725

				134.37		100.3725

				134.39		100.3725

				134.41		100.3686

				134.43		100.3686

				134.45		100.3686

				134.47		100.3686

				134.49		100.3686

				134.52		100.3686

				134.54		100.3686

				134.56		100.3686

				134.58		100.3686

				134.6		100.3686

				134.62		100.3686

				134.64		100.3686

				134.66		100.3686

				134.69		100.3686

				134.71		100.3686

				134.73		100.3686

				134.75		100.3686

				134.77		100.3686

				134.79		100.3686

				134.81		100.3686

				134.83		100.3686

				134.85		100.3686

				134.88		100.3686

				134.9		100.3647

				134.92		100.3647

				134.94		100.3686

				134.96		100.3686

				134.98		100.3647

				135		100.3686

				135.02		100.3647

				135.04		100.3647

				135.07		100.3647

				135.09		100.3647

				135.11		100.3686

				135.13		100.3647

				135.15		100.3647

				135.17		100.3647

				135.19		100.3647

				135.21		100.3647

				135.24		100.3647

				135.26		100.3647

				135.28		100.3647

				135.3		100.3647

				135.32		100.3608

				135.34		100.3647

				135.36		100.3608

				135.38		100.3608

				135.4		100.3608

				135.43		100.3608

				135.45		100.3608

				135.47		100.3608

				135.49		100.3608

				135.51		100.3608

				135.53		100.3608

				135.55		100.3608

				135.57		100.3608

				135.59		100.3608

				135.62		100.3608

				135.64		100.3608

				135.66		100.3608

				135.68		100.3608

				135.7		100.357

				135.72		100.357

				135.74		100.357

				135.76		100.357

				135.79		100.357

				135.81		100.357

				135.83		100.357

				135.85		100.357

				135.87		100.357

				135.89		100.357

				135.91		100.3531

				135.93		100.3531

				135.95		100.3531

				135.98		100.3531

				136		100.3531

				136.02		100.3531

				136.04		100.3531

				136.06		100.3531

				136.08		100.3531

				136.1		100.3531

				136.12		100.3531

				136.14		100.3531

				136.17		100.3531

				136.19		100.3531

				136.21		100.3531

				136.23		100.3531

				136.25		100.3531

				136.27		100.3531

				136.29		100.3531

				136.31		100.3531

				136.34		100.3531

				136.36		100.3531

				136.38		100.3531

				136.4		100.3531

				136.42		100.3492

				136.44		100.3492

				136.46		100.3492

				136.48		100.3492

				136.5		100.3492

				136.53		100.3492

				136.55		100.3492

				136.57		100.3492

				136.59		100.3492

				136.61		100.3492

				136.63		100.3492

				136.65		100.3492

				136.67		100.3492

				136.7		100.3492

				136.72		100.3492

				136.74		100.3492

				136.76		100.3492

				136.78		100.3453

				136.8		100.3492

				136.82		100.3492

				136.84		100.3453

				136.86		100.3453

				136.89		100.3453

				136.91		100.3453

				136.93		100.3453

				136.95		100.3453

				136.97		100.3453

				136.99		100.3453

				137.01		100.3453

				137.03		100.3453

				137.06		100.3414

				137.08		100.3453

				137.1		100.3414

				137.12		100.3414

				137.14		100.3414

				137.16		100.3414

				137.18		100.3414

				137.2		100.3414

				137.22		100.3414

				137.25		100.3414

				137.27		100.3414

				137.29		100.3376

				137.31		100.3376

				137.33		100.3376

				137.35		100.3376

				137.37		100.3376

				137.39		100.3376

				137.42		100.3376

				137.44		100.3376

				137.46		100.3376

				137.48		100.3376

				137.5		100.3376

				137.52		100.3376

				137.54		100.3376

				137.56		100.3376

				137.58		100.3376

				137.61		100.3376

				137.63		100.3376

				137.65		100.3337

				137.67		100.3376

				137.69		100.3376

				137.71		100.3337

				137.73		100.3376

				137.75		100.3337

				137.77		100.3337

				137.8		100.3337

				137.82		100.3337

				137.84		100.3337

				137.86		100.3337

				137.88		100.3337

				137.9		100.3337

				137.92		100.3337

				137.94		100.3337

				137.97		100.3337

				137.99		100.3337

				138.01		100.3337

				138.03		100.3298

				138.05		100.3337

				138.07		100.3298

				138.09		100.3298

				138.11		100.3298

				138.13		100.3298

				138.16		100.3298

				138.18		100.3298

				138.2		100.3298

				138.22		100.3298

				138.24		100.3298

				138.26		100.3298

				138.28		100.3298

				138.3		100.3298

				138.32		100.3259

				138.35		100.3259

				138.37		100.3259

				138.39		100.3259

				138.41		100.3259

				138.43		100.3259

				138.45		100.3259

				138.47		100.3259

				138.49		100.3259

				138.52		100.3259

				138.54		100.3259

				138.56		100.3259

				138.58		100.3259

				138.6		100.3259

				138.62		100.3259

				138.64		100.3259

				138.66		100.3259

				138.68		100.3259

				138.71		100.3259

				138.73		100.322

				138.75		100.3259

				138.77		100.3259

				138.79		100.3259

				138.81		100.322

				138.83		100.322

				138.85		100.322

				138.87		100.322

				138.9		100.322

				138.92		100.322

				138.94		100.322

				138.96		100.322

				138.98		100.322

				139		100.322

				139.02		100.322

				139.04		100.322

				139.07		100.322

				139.09		100.322

				139.11		100.322

				139.13		100.322

				139.15		100.322

				139.17		100.322

				139.19		100.322

				139.21		100.322

				139.23		100.322

				139.26		100.322

				139.28		100.322

				139.3		100.322

				139.32		100.322

				139.34		100.322

				139.36		100.322

				139.38		100.322

				139.4		100.322

				139.43		100.322

				139.45		100.322

				139.47		100.322

				139.49		100.322

				139.51		100.322

				139.53		100.322

				139.55		100.322

				139.57		100.322

				139.59		100.322

				139.62		100.322

				139.64		100.322

				139.66		100.322

				139.68		100.322

				139.7		100.322

				139.72		100.322

				139.74		100.322

				139.76		100.3182

				139.78		100.3182

				139.81		100.3182

				139.83		100.3182

				139.85		100.3182

				139.87		100.3182

				139.89		100.3182

				139.91		100.3182

				139.93		100.3182

				139.95		100.3182

				139.98		100.3182

				140		100.3182

				140.02		100.3182

				140.04		100.3182

				140.06		100.3182

				140.08		100.3182

				140.1		100.3182

				140.12		100.3182

				140.14		100.3182

				140.17		100.3182

				140.19		100.3182

				140.21		100.3182

				140.23		100.3143

				140.25		100.3143

				140.27		100.3143

				140.29		100.3143

				140.31		100.3143

				140.33		100.3143

				140.36		100.3143

				140.38		100.3143

				140.4		100.3143

				140.42		100.3143

				140.44		100.3143

				140.46		100.3143

				140.48		100.3143

				140.5		100.3143

				140.53		100.3143

				140.55		100.3143

				140.57		100.3143

				140.59		100.3143

				140.61		100.3143

				140.63		100.3143

				140.65		100.3143

				140.67		100.3104

				140.69		100.3104

				140.72		100.3104

				140.74		100.3104

				140.76		100.3104

				140.78		100.3104

				140.8		100.3104

				140.82		100.3104

				140.84		100.3104

				140.86		100.3065

				140.89		100.3065

				140.91		100.3104

				140.93		100.3065

				140.95		100.3065

				140.97		100.3065

				140.99		100.3065

				141.01		100.3065

				141.03		100.3065

				141.05		100.3065

				141.08		100.3065

				141.1		100.3065

				141.12		100.3065

				141.14		100.3065

				141.16		100.3065

				141.18		100.3026

				141.2		100.3065

				141.22		100.3026

				141.24		100.3026

				141.27		100.3026

				141.29		100.3026

				141.31		100.3026

				141.33		100.3026

				141.35		100.3026

				141.37		100.3026

				141.39		100.3026

				141.41		100.3026

				141.44		100.3026

				141.46		100.2988

				141.48		100.2988

				141.5		100.3026

				141.52		100.3026

				141.54		100.3026

				141.56		100.3026

				141.58		100.3026

				141.6		100.2988

				141.63		100.2988

				141.65		100.2988

				141.67		100.2988

				141.69		100.2988

				141.71		100.2988

				141.73		100.2988

				141.75		100.2988

				141.77		100.2988

				141.8		100.2949

				141.82		100.2949

				141.84		100.2988

				141.86		100.2949

				141.88		100.2949

				141.9		100.2949

				141.92		100.2949

				141.94		100.2949

				141.96		100.2949

				141.99		100.2949

				142.01		100.2949

				142.03		100.2949

				142.05		100.2949

				142.07		100.2949

				142.09		100.2949

				142.11		100.2949

				142.13		100.2949

				142.16		100.291

				142.18		100.291

				142.2		100.291

				142.22		100.291

				142.24		100.291

				142.26		100.291

				142.28		100.291

				142.3		100.291

				142.33		100.291

				142.35		100.291

				142.37		100.291

				142.39		100.291

				142.41		100.291

				142.43		100.2871

				142.45		100.291

				142.47		100.2871

				142.5		100.2871

				142.52		100.2871

				142.54		100.2871

				142.56		100.2871

				142.58		100.2871

				142.6		100.2871

				142.62		100.2871

				142.64		100.2871

				142.66		100.2832

				142.69		100.2832

				142.71		100.2832

				142.73		100.2832

				142.75		100.2832

				142.77		100.2832

				142.79		100.2832

				142.81		100.2832

				142.83		100.2832

				142.86		100.2832

				142.88		100.2832

				142.9		100.2832

				142.92		100.2832

				142.94		100.2832

				142.96		100.2794

				142.98		100.2794

				143		100.2794

				143.02		100.2794

				143.05		100.2794

				143.07		100.2794

				143.09		100.2794

				143.11		100.2794

				143.13		100.2794

				143.15		100.2755

				143.17		100.2755

				143.19		100.2755

				143.22		100.2755

				143.24		100.2755

				143.26		100.2755

				143.28		100.2755

				143.3		100.2755

				143.32		100.2755

				143.34		100.2755

				143.36		100.2755

				143.39		100.2716

				143.41		100.2716

				143.43		100.2716

				143.45		100.2716

				143.47		100.2716

				143.49		100.2716

				143.51		100.2716

				143.53		100.2716

				143.55		100.2716

				143.58		100.2677

				143.6		100.2677

				143.62		100.2677

				143.64		100.2677

				143.66		100.2677

				143.68		100.2677

				143.7		100.2677

				143.72		100.2638

				143.75		100.2638

				143.77		100.2638

				143.79		100.2677

				143.81		100.2638

				143.83		100.2638

				143.85		100.2638

				143.87		100.2638

				143.89		100.2638

				143.92		100.26

				143.94		100.26

				143.96		100.26

				143.98		100.26

				144		100.26

				144.02		100.26

				144.04		100.26

				144.06		100.26

				144.08		100.26

				144.11		100.2561

				144.13		100.2561

				144.15		100.2561

				144.17		100.2561

				144.19		100.2561

				144.21		100.2561

				144.23		100.2561

				144.25		100.2561

				144.28		100.2561

				144.3		100.2561

				144.32		100.2561

				144.34		100.2561

				144.36		100.2561

				144.38		100.2561

				144.4		100.2561

				144.42		100.2522

				144.45		100.2522

				144.47		100.2522

				144.49		100.2522

				144.51		100.2522

				144.53		100.2561

				144.55		100.2522

				144.57		100.2522

				144.59		100.2522

				144.62		100.2522

				144.64		100.2522

				144.66		100.2522

				144.68		100.2522

				144.7		100.2522

				144.72		100.2522

				144.74		100.2522

				144.76		100.2522

				144.78		100.2483

				144.81		100.2522

				144.83		100.2522

				144.85		100.2483

				144.87		100.2483

				144.89		100.2483

				144.91		100.2483

				144.93		100.2483

				144.95		100.2483

				144.98		100.2483

				145		100.2483

				145.02		100.2483

				145.04		100.2483

				145.06		100.2483

				145.08		100.2483

				145.1		100.2483

				145.12		100.2483

				145.15		100.2483

				145.17		100.2444

				145.19		100.2444

				145.21		100.2444

				145.23		100.2444

				145.25		100.2444

				145.27		100.2444

				145.29		100.2444

				145.32		100.2444

				145.34		100.2444

				145.36		100.2444

				145.38		100.2444

				145.4		100.2444

				145.42		100.2444

				145.44		100.2406

				145.46		100.2444

				145.49		100.2406

				145.51		100.2406

				145.53		100.2406

				145.55		100.2406

				145.57		100.2406

				145.59		100.2406

				145.61		100.2406

				145.63		100.2406

				145.65		100.2406

				145.68		100.2406

				145.7		100.2406

				145.72		100.2367

				145.74		100.2367

				145.76		100.2367

				145.78		100.2367

				145.8		100.2367

				145.82		100.2367

				145.85		100.2406

				145.87		100.2367

				145.89		100.2367

				145.91		100.2367

				145.93		100.2367

				145.95		100.2367

				145.97		100.2367

				145.99		100.2367

				146.02		100.2367

				146.04		100.2367

				146.06		100.2367

				146.08		100.2367

				146.1		100.2367

				146.12		100.2367

				146.14		100.2367

				146.16		100.2367

				146.19		100.2367

				146.21		100.2367

				146.23		100.2367

				146.25		100.2367

				146.27		100.2328

				146.29		100.2328

				146.31		100.2328

				146.33		100.2328

				146.35		100.2328

				146.38		100.2328

				146.4		100.2328

				146.42		100.2328

				146.44		100.2328

				146.46		100.2328

				146.48		100.2328

				146.5		100.2289

				146.52		100.2289

				146.55		100.2289

				146.57		100.2289

				146.59		100.2289

				146.61		100.2289

				146.63		100.2289

				146.65		100.2289

				146.67		100.2289

				146.69		100.2289

				146.72		100.2289

				146.74		100.2289

				146.76		100.225

				146.78		100.225

				146.8		100.225

				146.82		100.225

				146.84		100.225

				146.86		100.225

				146.89		100.225

				146.91		100.225

				146.93		100.225

				146.95		100.225

				146.97		100.2212

				146.99		100.2212

				147.01		100.2212

				147.03		100.2212

				147.05		100.2212

				147.08		100.2212

				147.1		100.2212

				147.12		100.2212

				147.14		100.2212

				147.16		100.2173

				147.18		100.2212

				147.2		100.2173

				147.22		100.2173

				147.25		100.2173

				147.27		100.2173

				147.29		100.2173

				147.31		100.2173

				147.33		100.2173

				147.35		100.2173

				147.37		100.2173

				147.39		100.2134

				147.42		100.2134

				147.44		100.2134

				147.46		100.2134

				147.48		100.2134

				147.5		100.2134

				147.52		100.2134

				147.54		100.2134

				147.56		100.2134

				147.59		100.2134

				147.61		100.2095

				147.63		100.2134

				147.65		100.2095

				147.67		100.2095

				147.69		100.2095

				147.71		100.2095

				147.73		100.2095

				147.76		100.2095

				147.78		100.2095

				147.8		100.2095

				147.82		100.2056

				147.84		100.2056

				147.86		100.2056

				147.88		100.2056

				147.9		100.2056

				147.93		100.2056

				147.95		100.2056

				147.97		100.2056

				147.99		100.2056

				148.01		100.2018

				148.03		100.2018

				148.05		100.2018

				148.07		100.2018

				148.1		100.2018

				148.12		100.2018

				148.14		100.2018

				148.16		100.2018

				148.18		100.1979

				148.2		100.1979

				148.22		100.1979

				148.24		100.1979

				148.27		100.1979

				148.29		100.194

				148.31		100.1979

				148.33		100.194

				148.35		100.194

				148.37		100.194

				148.39		100.194

				148.41		100.194

				148.44		100.194

				148.46		100.194

				148.48		100.194

				148.5		100.194

				148.52		100.194

				148.54		100.194

				148.56		100.1901

				148.58		100.1901

				148.61		100.1901

				148.63		100.1901

				148.65		100.1901

				148.67		100.1901

				148.69		100.1901

				148.71		100.1901

				148.73		100.1901

				148.75		100.1901

				148.78		100.1901

				148.8		100.1901

				148.82		100.1862

				148.84		100.1862

				148.86		100.1862

				148.88		100.1862

				148.9		100.1862

				148.92		100.1862

				148.95		100.1862

				148.97		100.1862

				148.99		100.1862

				149.01		100.1862

				149.03		100.1862

				149.05		100.1824

				149.07		100.1824

				149.09		100.1824

				149.11		100.1824

				149.14		100.1824

				149.16		100.1824

				149.18		100.1824

				149.2		100.1824

				149.22		100.1824

				149.24		100.1785

				149.26		100.1824

				149.28		100.1785

				149.31		100.1785

				149.33		100.1785

				149.35		100.1785

				149.37		100.1785

				149.39		100.1785

				149.41		100.1785

				149.43		100.1785

				149.45		100.1785

				149.48		100.1785

				149.5		100.1785

				149.52		100.1746

				149.54		100.1746

				149.56		100.1746

				149.58		100.1746

				149.6		100.1746

				149.62		100.1746

				149.64		100.1746

				149.67		100.1746

				149.69		100.1746

				149.71		100.1746

				149.73		100.1746

				149.75		100.1746

				149.77		100.1707

				149.79		100.1707

				149.81		100.1707

				149.84		100.1707

				149.86		100.1707

				149.88		100.1707

				149.9		100.1707

				149.92		100.1707

				149.94		100.1707

				149.96		100.1707

				149.98		100.1668

				150.01		100.1668

				150.03		100.1668

				150.05		100.1668

				150.07		100.1668

				150.09		100.1668

				150.11		100.1668

				150.13		100.1668

				150.15		100.1668

				150.17		100.1668

				150.2		100.1668

				150.22		100.1668

				150.24		100.1668

				150.26		100.163

				150.28		100.163

				150.3		100.163

				150.32		100.163

				150.34		100.163

				150.37		100.163

				150.39		100.163

				150.41		100.163

				150.43		100.163

				150.45		100.163

				150.47		100.163

				150.49		100.163

				150.51		100.163

				150.54		100.163

				150.56		100.1591

				150.58		100.1591

				150.6		100.1591

				150.62		100.1591

				150.64		100.1591

				150.66		100.1591

				150.68		100.1552

				150.7		100.1552

				150.73		100.1552

				150.75		100.1552

				150.77		100.1552

				150.79		100.1552

				150.81		100.1552

				150.83		100.1552

				150.85		100.1552

				150.87		100.1513

				150.9		100.1513

				150.92		100.1513

				150.94		100.1513

				150.96		100.1513

				150.98		100.1513

				151		100.1474

				151.02		100.1474

				151.04		100.1474

				151.07		100.1474

				151.09		100.1474

				151.11		100.1474

				151.13		100.1474

				151.15		100.1474

				151.17		100.1436

				151.19		100.1436

				151.21		100.1436

				151.24		100.1436

				151.26		100.1436

				151.28		100.1436

				151.3		100.1436

				151.32		100.1397

				151.34		100.1397

				151.36		100.1397

				151.38		100.1397

				151.4		100.1397

				151.43		100.1397

				151.45		100.1397

				151.47		100.1397

				151.49		100.1358

				151.51		100.1358

				151.53		100.1358

				151.55		100.1358

				151.57		100.1358

				151.6		100.1358

				151.62		100.1358

				151.64		100.1319

				151.66		100.1319

				151.68		100.1319

				151.7		100.1319

				151.72		100.1319

				151.74		100.1319

				151.77		100.1319

				151.79		100.1319

				151.81		100.1319

				151.83		100.128

				151.85		100.128

				151.87		100.128

				151.89		100.128

				151.91		100.128

				151.93		100.1242

				151.96		100.1242

				151.98		100.1242

				152		100.1203

				152.02		100.1203

				152.04		100.1203

				152.06		100.1203

				152.08		100.1203

				152.1		100.1164

				152.13		100.1164

				152.15		100.1164

				152.17		100.1164

				152.19		100.1164

				152.21		100.1164

				152.23		100.1164

				152.25		100.1164

				152.27		100.1125

				152.3		100.1125

				152.32		100.1125

				152.34		100.1086

				152.36		100.1086

				152.38		100.1086

				152.4		100.1086

				152.42		100.1086

				152.44		100.1048

				152.46		100.1048

				152.49		100.1048

				152.51		100.1048

				152.53		100.1048

				152.55		100.1009

				152.57		100.1009

				152.59		100.1009

				152.61		100.1009

				152.63		100.1009

				152.66		100.1009

				152.68		100.1009

				152.7		100.1009

				152.72		100.097

				152.74		100.097

				152.76		100.097

				152.78		100.097

				152.8		100.097

				152.83		100.0931

				152.85		100.0931

				152.87		100.0931

				152.89		100.0931

				152.91		100.0931

				152.93		100.0931

				152.95		100.0931

				152.97		100.0931

				152.99		100.0931

				153.02		100.0931

				153.04		100.0892

				153.06		100.0892

				153.08		100.0892

				153.1		100.0892

				153.12		100.0892

				153.14		100.0854

				153.16		100.0854

				153.19		100.0854

				153.21		100.0854

				153.23		100.0854

				153.25		100.0815

				153.27		100.0815

				153.29		100.0815

				153.31		100.0815

				153.33		100.0815

				153.35		100.0815

				153.38		100.0815

				153.4		100.0815

				153.42		100.0815

				153.44		100.0776

				153.46		100.0776

				153.48		100.0776

				153.5		100.0776

				153.52		100.0776

				153.55		100.0776

				153.57		100.0737

				153.59		100.0737

				153.61		100.0737

				153.63		100.0737

				153.65		100.0737

				153.67		100.0737

				153.69		100.0737

				153.71		100.0737

				153.74		100.0698

				153.76		100.0698

				153.78		100.0698

				153.8		100.0698

				153.82		100.0698

				153.84		100.0698

				153.86		100.066

				153.88		100.066

				153.91		100.066

				153.93		100.0621

				153.95		100.0621

				153.97		100.0621

				153.99		100.0582

				154.01		100.0582

				154.03		100.0582

				154.05		100.0582

				154.07		100.0582

				154.1		100.0582

				154.12		100.0582

				154.14		100.0543

				154.16		100.0543

				154.18		100.0543

				154.2		100.0504

				154.22		100.0504

				154.24		100.0504

				154.27		100.0504

				154.29		100.0466

				154.31		100.0466

				154.33		100.0466

				154.35		100.0466

				154.37		100.0466

				154.39		100.0427

				154.41		100.0427

				154.43		100.0427

				154.46		100.0388

				154.48		100.0388

				154.5		100.0388

				154.52		100.0388

				154.54		100.0388

				154.56		100.0388

				154.58		100.0388

				154.6		100.0349

				154.63		100.0388

				154.65		100.0349

				154.67		100.0349

				154.69		100.0349

				154.71		100.0349

				154.73		100.0349

				154.75		100.0349

				154.77		100.031

				154.79		100.031

				154.82		100.031

				154.84		100.0272

				154.86		100.0272

				154.88		100.0272

				154.9		100.0272

				154.92		100.0233

				154.94		100.0233

				154.96		100.0233

				154.99		100.0233

				155.01		100.0233

				155.03		100.0194

				155.05		100.0194

				155.07		100.0194

				155.09		100.0194

				155.11		100.0194

				155.13		100.0194

				155.15		100.0194

				155.18		100.0155

				155.2		100.0194

				155.22		100.0194

				155.24		100.0155

				155.26		100.0155

				155.28		100.0155

				155.3		100.0155

				155.32		100.0116

				155.35		100.0116

				155.37		100.0116

				155.39		100.0116

				155.41		100.0078

				155.43		100.0078

				155.45		100.0078

				155.47		100.0078

				155.49		100.0039

				155.51		100.0039

				155.54		100.0039

				155.56		100.0039

				155.58		100.0039

				155.6		100.0039

				155.62		100.0039

				155.64		100.0039

				155.66		100.0039

				155.68		100.0039

				155.71		100

				155.73		100

				155.75		100

				155.77		100

				155.79		100

				155.81		99.99612

				155.83		99.99612

				155.85		99.99612

				155.87		99.99612

				155.9		99.99612

				155.92		99.99224

				155.94		99.99224

				155.96		99.99224

				155.98		99.99224

				156		99.99224

				156.02		99.98836

				156.04		99.98836

				156.06		99.98836

				156.09		99.98836

				156.11		99.98836

				156.13		99.98448

				156.15		99.98448

				156.17		99.98448

				156.19		99.98448

				156.21		99.98448

				156.23		99.98448

				156.26		99.98448

				156.28		99.9806

				156.3		99.9806

				156.32		99.9806

				156.34		99.9806

				156.36		99.9806

				156.38		99.97672

				156.4		99.97672

				156.42		99.97672

				156.45		99.97284

				156.47		99.97284

				156.49		99.97284

				156.51		99.97284

				156.53		99.97284

				156.55		99.97284

				156.57		99.97284

				156.59		99.96896

				156.62		99.96896

				156.64		99.96896

				156.66		99.96896

				156.68		99.96896

				156.7		99.96896

				156.72		99.96508

				156.74		99.96896

				156.76		99.96896

				156.78		99.96508

				156.81		99.96508

				156.83		99.96508

				156.85		99.96508

				156.87		99.96508

				156.89		99.96508

				156.91		99.96508

				156.93		99.9612

				156.95		99.9612

				156.97		99.9612

				157		99.9612

				157.02		99.9612

				157.04		99.9612

				157.06		99.9612

				157.08		99.95732

				157.1		99.9612

				157.12		99.95732

				157.14		99.95732

				157.17		99.95732

				157.19		99.95344

				157.21		99.95344

				157.23		99.95344

				157.25		99.95344

				157.27		99.95344

				157.29		99.95344

				157.31		99.95344

				157.33		99.94956

				157.36		99.94956

				157.38		99.94956

				157.4		99.94956

				157.42		99.94956

				157.44		99.94568

				157.46		99.94568

				157.48		99.94568

				157.5		99.94568

				157.52		99.94568

				157.55		99.94568

				157.57		99.9418

				157.59		99.9418

				157.61		99.9418

				157.63		99.9418

				157.65		99.9418

				157.67		99.9418

				157.69		99.93792

				157.71		99.93792

				157.74		99.93792

				157.76		99.93404

				157.78		99.93404

				157.8		99.93404

				157.82		99.93404

				157.84		99.93016

				157.86		99.93016

				157.88		99.93016

				157.9		99.93016

				157.93		99.93016

				157.95		99.92628

				157.97		99.92628

				157.99		99.92628

				158.01		99.92628

				158.03		99.9224

				158.05		99.9224

				158.07		99.9224

				158.09		99.9224

				158.12		99.91852

				158.14		99.91852

				158.16		99.91852

				158.18		99.91464

				158.2		99.91464

				158.22		99.91464

				158.24		99.91464

				158.26		99.91464

				158.29		99.91076

				158.31		99.91076

				158.33		99.91076

				158.35		99.90688

				158.37		99.90688

				158.39		99.90688

				158.41		99.90688

				158.43		99.90688

				158.45		99.903

				158.48		99.903

				158.5		99.903

				158.52		99.89912

				158.54		99.89912

				158.56		99.89912

				158.58		99.89912

				158.6		99.89912

				158.62		99.89524

				158.64		99.89524

				158.67		99.89524

				158.69		99.89524

				158.71		99.89136

				158.73		99.89136

				158.75		99.89136

				158.77		99.89136

				158.79		99.88748

				158.81		99.88748

				158.83		99.88748

				158.86		99.88748

				158.88		99.88748

				158.9		99.88748

				158.92		99.88748

				158.94		99.88748

				158.96		99.8836

				158.98		99.8836

				159		99.8836

				159.03		99.8836

				159.05		99.8836

				159.07		99.87972

				159.09		99.87972

				159.11		99.87972

				159.13		99.87972

				159.15		99.87972

				159.17		99.87972

				159.19		99.87972

				159.22		99.87584

				159.24		99.87584

				159.26		99.87584

				159.28		99.87584

				159.3		99.87584

				159.32		99.87196

				159.34		99.87196

				159.36		99.87196

				159.38		99.87196

				159.41		99.86808

				159.43		99.86808

				159.45		99.8642

				159.47		99.8642

				159.49		99.8642

				159.51		99.8642

				159.53		99.8642

				159.55		99.86032

				159.57		99.86032

				159.6		99.86032

				159.62		99.86032

				159.64		99.86032

				159.66		99.85644

				159.68		99.85644

				159.7		99.85644

				159.72		99.85644

				159.74		99.85256

				159.77		99.85256

				159.79		99.85256

				159.81		99.85256

				159.83		99.85256

				159.85		99.85256

				159.87		99.85256

				159.89		99.84868

				159.91		99.84868

				159.93		99.84868

				159.96		99.84868

				159.98		99.8448

				160		99.8448

				160.02		99.8448

				160.04		99.8448

				160.06		99.84092

				160.08		99.84092

				160.1		99.84092

				160.12		99.84092

				160.15		99.84092

				160.17		99.83704

				160.19		99.83704

				160.21		99.83704

				160.23		99.83704

				160.25		99.83316

				160.27		99.83316

				160.29		99.83316

				160.31		99.82928

				160.34		99.82928

				160.36		99.82928

				160.38		99.8254

				160.4		99.8254

				160.42		99.8254

				160.44		99.82152

				160.46		99.8254

				160.48		99.82152

				160.5		99.82152

				160.53		99.82152

				160.55		99.82152

				160.57		99.82152

				160.59		99.82152

				160.61		99.81764

				160.63		99.82152

				160.65		99.81764

				160.67		99.81764

				160.69		99.81764

				160.72		99.81376

				160.74		99.81376

				160.76		99.81376

				160.78		99.81376

				160.8		99.80988

				160.82		99.80988

				160.84		99.80988

				160.86		99.80988

				160.88		99.80988

				160.91		99.806

				160.93		99.806

				160.95		99.80212

				160.97		99.80212

				160.99		99.80212

				161.01		99.79824

				161.03		99.79824

				161.05		99.79824

				161.07		99.79824

				161.1		99.79824

				161.12		99.79436

				161.14		99.79436

				161.16		99.79436

				161.18		99.79436

				161.2		99.79048

				161.22		99.79048

				161.24		99.79048

				161.26		99.7866

				161.29		99.7866

				161.31		99.7866

				161.33		99.7866

				161.35		99.78272

				161.37		99.78272

				161.39		99.78272

				161.41		99.77884

				161.43		99.77884

				161.45		99.77884

				161.48		99.77496

				161.5		99.77108

				161.52		99.77108

				161.54		99.77108

				161.56		99.7672

				161.58		99.7672

				161.6		99.7672

				161.62		99.76332

				161.64		99.76332

				161.67		99.76332

				161.69		99.75944

				161.71		99.75944

				161.73		99.75944

				161.75		99.75944

				161.77		99.75944

				161.79		99.75556

				161.81		99.75556

				161.83		99.75556

				161.86		99.75556

				161.88		99.75556

				161.9		99.75168

				161.92		99.75168

				161.94		99.75556

				161.96		99.75168

				161.98		99.75168

				162		99.75168

				162.02		99.7478

				162.05		99.7478

				162.07		99.7478

				162.09		99.7478

				162.11		99.74392

				162.13		99.74392

				162.15		99.74392

				162.17		99.74004

				162.19		99.74004

				162.21		99.73616

				162.23		99.73616

				162.26		99.73616

				162.28		99.73616

				162.3		99.73616

				162.32		99.73616

				162.34		99.73228

				162.36		99.73616

				162.38		99.73228

				162.4		99.73228

				162.42		99.73228

				162.45		99.73228

				162.47		99.73228

				162.49		99.73228

				162.51		99.73228

				162.53		99.7284

				162.55		99.7284

				162.57		99.7284

				162.59		99.7284

				162.61		99.72452

				162.64		99.72452

				162.66		99.72452

				162.68		99.72064

				162.7		99.71676

				162.72		99.71676

				162.74		99.71288

				162.76		99.71288

				162.78		99.71288

				162.8		99.71288

				162.83		99.71288

				162.85		99.709

				162.87		99.709

				162.89		99.709

				162.91		99.709

				162.93		99.709

				162.95		99.70512

				162.97		99.70512

				162.99		99.70512

				163.02		99.70124

				163.04		99.70512

				163.06		99.70124

				163.08		99.70124

				163.1		99.70124

				163.12		99.70512

				163.14		99.70124

				163.16		99.70124

				163.18		99.69736

				163.21		99.69348

				163.23		99.69348

				163.25		99.6896

				163.27		99.6896

				163.29		99.6896

				163.31		99.68572

				163.33		99.6896

				163.35		99.68572

				163.37		99.68572

				163.4		99.68572

				163.42		99.68572

				163.44		99.68572

				163.46		99.68184

				163.48		99.68184

				163.5		99.68184

				163.52		99.68184

				163.54		99.68184

				163.56		99.68184

				163.59		99.68184

				163.61		99.68184

				163.63		99.68184

				163.65		99.68184

				163.67		99.67796

				163.69		99.67796

				163.71		99.67408

				163.73		99.67408

				163.75		99.67408

				163.78		99.6702

				163.8		99.66632

				163.82		99.6702

				163.84		99.66632

				163.86		99.66244

				163.88		99.66244

				163.9		99.65856

				163.92		99.65856

				163.94		99.65856

				163.97		99.65468

				163.99		99.65468

				164.01		99.65468

				164.03		99.65856

				164.05		99.65856

				164.07		99.65468

				164.09		99.65856

				164.11		99.65856

				164.13		99.65468

				164.15		99.65468

				164.18		99.6508

				164.2		99.64692

				164.22		99.64692

				164.24		99.64692

				164.26		99.63916

				164.28		99.63528

				164.3		99.6314

				164.32		99.6314

				164.34		99.62752

				164.37		99.62752

				164.39		99.62364

				164.41		99.62364

				164.43		99.62364

				164.45		99.62364

				164.47		99.62364

				164.49		99.61976

				164.51		99.62364

				164.53		99.61976

				164.56		99.61976

				164.58		99.61588

				164.6		99.61976

				164.62		99.61588

				164.64		99.61588

				164.66		99.612

				164.68		99.612

				164.7		99.612

				164.72		99.60812

				164.75		99.612

				164.77		99.60812

				164.79		99.60812

				164.81		99.60812

				164.83		99.60424

				164.85		99.60036

				164.87		99.59648

				164.89		99.60036

				164.91		99.60036

				164.94		99.59648

				164.96		99.59648

				164.98		99.59648

				165		99.60036

				165.02		99.59648

				165.04		99.59648

				165.06		99.59648

				165.08		99.59648

				165.1		99.5926

				165.13		99.59648

				165.15		99.5926

				165.17		99.5926

				165.19		99.5926

				165.21		99.5926

				165.23		99.58872

				165.25		99.58872

				165.27		99.58872

				165.29		99.58484

				165.31		99.58484

				165.34		99.58484

				165.36		99.58096

				165.38		99.58096

				165.4		99.57708

				165.42		99.58096

				165.44		99.57708

				165.46		99.57708

				165.48		99.5732

				165.5		99.5732

				165.53		99.5732

				165.55		99.5732

				165.57		99.5732

				165.59		99.56932

				165.61		99.56932

				165.63		99.56932

				165.65		99.56544

				165.67		99.56544

				165.69		99.56544

				165.72		99.56156

				165.74		99.56156

				165.76		99.5538

				165.78		99.5538

				165.8		99.5538

				165.82		99.5538

				165.84		99.54992

				165.86		99.5538

				165.88		99.5538

				165.91		99.54992

				165.93		99.54992

				165.95		99.5538

				165.97		99.54604

				165.99		99.54604

				166.01		99.54604

				166.03		99.54216

				166.05		99.53828

				166.07		99.53828

				166.09		99.5344

				166.12		99.5344

				166.14		99.5344

				166.16		99.5344

				166.18		99.53052

				166.2		99.53052

				166.22		99.53052

				166.24		99.53052

				166.26		99.52276

				166.28		99.52276

				166.31		99.52664

				166.33		99.51888

				166.35		99.51888

				166.37		99.51888

				166.39		99.51888

				166.41		99.51888

				166.43		99.51888

				166.45		99.51112

				166.47		99.515

				166.49		99.50724

				166.52		99.51112

				166.54		99.51112

				166.56		99.50724

				166.58		99.50724

				166.6		99.50336

				166.62		99.4956

				166.64		99.4956

				166.66		99.4956

				166.68		99.4956

				166.71		99.4956

				166.73		99.49172

				166.75		99.49172

				166.77		99.49172

				166.79		99.49172

				166.81		99.48784

				166.83		99.48784

				166.85		99.48396

				166.87		99.48396

				166.89		99.48784

				166.92		99.48396

				166.94		99.48396

				166.96		99.48784

				166.98		99.48396

				167		99.48396

				167.02		99.48396

				167.04		99.48008

				167.06		99.4762

				167.08		99.4762

				167.11		99.4762

				167.13		99.48008

				167.15		99.46844

				167.17		99.47232

				167.19		99.47232

				167.21		99.46456

				167.23		99.46844

				167.25		99.46456

				167.27		99.46456

				167.3		99.46068

				167.32		99.4568

				167.34		99.4568

				167.36		99.4568

				167.38		99.4568

				167.4		99.4568

				167.42		99.45292

				167.44		99.44904

				167.46		99.44516

				167.48		99.44516

				167.51		99.44516

				167.53		99.44516

				167.55		99.44127

				167.57		99.44127

				167.59		99.42963

				167.61		99.42575

				167.63		99.43739

				167.65		99.42187

				167.67		99.42963

				167.7		99.42963

				167.72		99.42575

				167.74		99.42575

				167.76		99.42187

				167.78		99.41799

				167.8		99.41799

				167.82		99.41799

				167.84		99.41799

				167.86		99.41411

				167.88		99.41411

				167.91		99.41411

				167.93		99.41799

				167.95		99.41411

				167.97		99.41023

				167.99		99.41023

				168.01		99.40635

				168.03		99.40635

				168.05		99.40635

				168.07		99.40635

				168.1		99.40635

				168.12		99.39859

				168.14		99.39859

				168.16		99.39859

				168.18		99.40247

				168.2		99.39859

				168.22		99.38307

				168.24		99.39471

				168.26		99.38307

				168.28		99.38307

				168.31		99.38307

				168.33		99.38307

				168.35		99.37919

				168.37		99.37919

				168.39		99.37531

				168.41		99.37531

				168.43		99.37531

				168.45		99.37143

				168.47		99.36755

				168.5		99.36755

				168.52		99.36367

				168.54		99.36367

				168.56		99.36367

				168.58		99.35979

				168.6		99.35979

				168.62		99.35979

				168.64		99.35591

				168.66		99.35591

				168.68		99.35203

				168.71		99.35203

				168.73		99.35203

				168.75		99.34815

				168.77		99.34815

				168.79		99.34815

				168.81		99.34815

				168.83		99.34427

				168.85		99.34427

				168.87		99.34427

				168.9		99.34039

				168.92		99.33651

				168.94		99.33651

				168.96		99.33651

				168.98		99.33651

				169		99.34039

				169.02		99.33651

				169.04		99.33263

				169.06		99.33263

				169.08		99.33263

				169.11		99.32875

				169.13		99.32875

				169.15		99.33263

				169.17		99.32875

				169.19		99.32487

				169.21		99.32487

				169.23		99.32099

				169.25		99.31711

				169.27		99.31711

				169.29		99.31711

				169.32		99.31323

				169.34		99.30935

				169.36		99.30935

				169.38		99.30935

				169.4		99.30547

				169.42		99.30547

				169.44		99.30547

				169.46		99.30159

				169.48		99.30159

				169.51		99.29771

				169.53		99.29771

				169.55		99.29771

				169.57		99.29383

				169.59		99.28995

				169.61		99.28995

				169.63		99.28607

				169.65		99.28607

				169.67		99.28219

				169.69		99.28219

				169.72		99.27443

				169.74		99.27055

				169.76		99.27055

				169.78		99.26667

				169.8		99.26279

				169.82		99.26667

				169.84		99.26279

				169.86		99.26279

				169.88		99.25891

				169.9		99.26279

				169.93		99.25503

				169.95		99.25503

				169.97		99.25503

				169.99		99.25115

				170.01		99.25115

				170.03		99.25115

				170.05		99.24727

				170.07		99.24727

				170.09		99.25115

				170.11		99.25115

				170.14		99.24727

				170.16		99.24727

				170.18		99.24339

				170.2		99.24339

				170.22		99.23951

				170.24		99.23951

				170.26		99.23563

				170.28		99.23563

				170.3		99.23175

				170.32		99.23563

				170.35		99.23175

				170.37		99.22787

				170.39		99.22787

				170.41		99.22787

				170.43		99.22399

				170.45		99.22399

				170.47		99.22399

				170.49		99.22399

				170.51		99.22011

				170.53		99.22011

				170.56		99.22011

				170.58		99.22011

				170.6		99.21623

				170.62		99.21623

				170.64		99.21623

				170.66		99.21623

				170.68		99.21623

				170.7		99.21623

				170.72		99.21235

				170.74		99.20847

				170.77		99.20847

				170.79		99.20459

				170.81		99.20459

				170.83		99.20071

				170.85		99.20071

				170.87		99.19683

				170.89		99.19295

				170.91		99.19295

				170.93		99.19295

				170.96		99.18907

				170.98		99.18907

				171		99.18907

				171.02		99.18907

				171.04		99.18519

				171.06		99.18519

				171.08		99.18907

				171.1		99.18519

				171.12		99.18519

				171.14		99.18519

				171.17		99.18131

				171.19		99.18131

				171.21		99.17743

				171.23		99.17743

				171.25		99.17355

				171.27		99.16967

				171.29		99.16579

				171.31		99.16191

				171.33		99.16191

				171.35		99.16191

				171.38		99.15803

				171.4		99.15803

				171.42		99.15415

				171.44		99.15415

				171.46		99.15415

				171.48		99.15415

				171.5		99.15415

				171.52		99.15415

				171.54		99.15415

				171.56		99.15027

				171.59		99.15027

				171.61		99.15027

				171.63		99.15027

				171.65		99.14639

				171.67		99.14251

				171.69		99.13863

				171.71		99.13863

				171.73		99.13863

				171.75		99.13863

				171.78		99.13863

				171.8		99.13475

				171.82		99.13087

				171.84		99.12311

				171.86		99.11923

				171.88		99.11923

				171.9		99.11535

				171.92		99.11147

				171.94		99.10759

				171.96		99.10759

				171.99		99.09983

				172.01		99.10371

				172.03		99.09983

				172.05		99.09983

				172.07		99.09595

				172.09		99.09595

				172.11		99.08819

				172.13		99.08819

				172.15		99.08819

				172.17		99.08431

				172.2		99.08431

				172.22		99.08043

				172.24		99.08043

				172.26		99.07655

				172.28		99.06879

				172.3		99.06879

				172.32		99.06879

				172.34		99.06879

				172.36		99.06879

				172.38		99.06879

				172.41		99.06491

				172.43		99.06879

				172.45		99.06491

				172.47		99.06491

				172.49		99.06491

				172.51		99.06491

				172.53		99.06103

				172.55		99.05715

				172.57		99.05715

				172.6		99.05715

				172.62		99.05327

				172.64		99.05327

				172.66		99.05327

				172.68		99.04939

				172.7		99.04551

				172.72		99.04551

				172.74		99.04939

				172.76		99.04551

				172.78		99.04551

				172.81		99.04551

				172.83		99.04163

				172.85		99.04163

				172.87		99.03775

				172.89		99.03775

				172.91		99.03775

				172.93		99.03387

				172.95		99.03387

				172.97		99.02999

				172.99		99.02611

				173.02		99.02611

				173.04		99.02223

				173.06		99.02223

				173.08		99.02223

				173.1		99.01835

				173.12		99.01835

				173.14		99.01447

				173.16		99.01447

				173.18		99.01447

				173.2		99.01447

				173.23		99.01059

				173.25		99.00671

				173.27		99.00671

				173.29		99.00283

				173.31		98.99895

				173.33		98.99507

				173.35		98.99507

				173.37		98.99119

				173.39		98.99119

				173.42		98.99119

				173.44		98.99507

				173.46		98.99119

				173.48		98.98731

				173.5		98.98343

				173.52		98.98343

				173.54		98.97955

				173.56		98.97955

				173.58		98.97955

				173.6		98.97955

				173.63		98.97567

				173.65		98.97179

				173.67		98.97179

				173.69		98.97179

				173.71		98.96791

				173.73		98.96403

				173.75		98.96403

				173.77		98.96015

				173.79		98.96015

				173.81		98.95627

				173.84		98.95627

				173.86		98.95627

				173.88		98.95239

				173.9		98.95239

				173.92		98.94851

				173.94		98.94851

				173.96		98.94463

				173.98		98.94463

				174		98.93687

				174.02		98.94075

				174.05		98.93299

				174.07		98.93687

				174.09		98.93687

				174.11		98.93687

				174.13		98.93299

				174.15		98.93299

				174.17		98.92911

				174.19		98.92911

				174.21		98.92523

				174.23		98.92523

				174.26		98.92135

				174.28		98.92135

				174.3		98.91747

				174.32		98.91747

				174.34		98.91747

				174.36		98.91359

				174.38		98.91359

				174.4		98.90971

				174.42		98.90583

				174.44		98.90195

				174.47		98.90195

				174.49		98.89807

				174.51		98.90195

				174.53		98.89419

				174.55		98.89419

				174.57		98.89031

				174.59		98.88643

				174.61		98.88255

				174.63		98.87867

				174.65		98.88255

				174.68		98.87867

				174.7		98.87867

				174.72		98.87479

				174.74		98.87479

				174.76		98.87479

				174.78		98.87091

				174.8		98.86703

				174.82		98.86315

				174.84		98.86315

				174.86		98.85539

				174.89		98.85539

				174.91		98.85539

				174.93		98.85151

				174.95		98.85151

				174.97		98.84763

				174.99		98.84763

				175.01		98.84375

				175.03		98.84375

				175.05		98.83987

				175.07		98.83987

				175.1		98.83599

				175.12		98.83599

				175.14		98.83211

				175.16		98.82823

				175.18		98.83211

				175.2		98.82435

				175.22		98.82435

				175.24		98.82435

				175.26		98.82047

				175.28		98.82047

				175.31		98.81659

				175.33		98.82047

				175.35		98.81659

				175.37		98.80883

				175.39		98.80883

				175.41		98.80883

				175.43		98.80495

				175.45		98.80495

				175.47		98.80107

				175.49		98.80107

				175.52		98.80107

				175.54		98.79719

				175.56		98.79331

				175.58		98.79331

				175.6		98.78943

				175.62		98.78943

				175.64		98.78555

				175.66		98.78555

				175.68		98.78167

				175.7		98.78167

				175.73		98.77779

				175.75		98.77391

				175.77		98.77391

				175.79		98.77391

				175.81		98.77391

				175.83		98.77003

				175.85		98.76615

				175.87		98.76227

				175.89		98.76227

				175.91		98.75839

				175.94		98.75839

				175.96		98.75451

				175.98		98.75451

				176		98.75063

				176.02		98.74675

				176.04		98.74675

				176.06		98.74287

				176.08		98.74287

				176.1		98.73899

				176.12		98.73511

				176.15		98.73123

				176.17		98.73123

				176.19		98.72735

				176.21		98.72735

				176.23		98.72347

				176.25		98.71959

				176.27		98.71959

				176.29		98.71959

				176.31		98.71571

				176.33		98.71571

				176.35		98.71183

				176.38		98.70795

				176.4		98.70795

				176.42		98.70019

				176.44		98.70019

				176.46		98.70019

				176.48		98.69631

				176.5		98.69243

				176.52		98.68855

				176.54		98.68855

				176.56		98.68467

				176.59		98.68079

				176.61		98.68079

				176.63		98.68079

				176.65		98.67303

				176.67		98.67691

				176.69		98.67303

				176.71		98.66915

				176.73		98.66527

				176.75		98.66527

				176.77		98.66139

				176.8		98.66139

				176.82		98.65751

				176.84		98.65751

				176.86		98.65363

				176.88		98.64975

				176.9		98.64975

				176.92		98.64975

				176.94		98.64975

				176.96		98.64587

				176.98		98.64199

				177.01		98.64199

				177.03		98.63811

				177.05		98.63423

				177.07		98.63423

				177.09		98.63035

				177.11		98.63035

				177.13		98.62647

				177.15		98.62259

				177.17		98.62259

				177.19		98.61871

				177.22		98.61483

				177.24		98.61871

				177.26		98.61871

				177.28		98.61483

				177.3		98.61095

				177.32		98.61095

				177.34		98.60707

				177.36		98.60319

				177.38		98.60319

				177.4		98.60319

				177.43		98.59931

				177.45		98.59155

				177.47		98.59155

				177.49		98.58767

				177.51		98.58379

				177.53		98.58379

				177.55		98.58379

				177.57		98.57603

				177.59		98.57215

				177.61		98.56439

				177.63		98.56439

				177.66		98.56051

				177.68		98.55663

				177.7		98.55275

				177.72		98.55663

				177.74		98.55275

				177.76		98.54887

				177.78		98.54499

				177.8		98.54111

				177.82		98.54111

				177.84		98.54499

				177.87		98.53335

				177.89		98.53335

				177.91		98.53723

				177.93		98.53335

				177.95		98.53335

				177.97		98.52559

				177.99		98.52171

				178.01		98.51783

				178.03		98.51783

				178.05		98.51007

				178.08		98.50619

				178.1		98.50231

				178.12		98.49843

				178.14		98.49455

				178.16		98.49843

				178.18		98.49843

				178.2		98.49843

				178.22		98.49455

				178.24		98.49067

				178.26		98.49843

				178.29		98.49067

				178.31		98.48679

				178.33		98.48679

				178.35		98.49067

				178.37		98.47903

				178.39		98.47903

				178.41		98.47903

				178.43		98.47903

				178.45		98.47903

				178.47		98.47515

				178.49		98.47127

				178.52		98.46351

				178.54		98.45575

				178.56		98.45575

				178.58		98.45187

				178.6		98.44799

				178.62		98.44799

				178.64		98.44023

				178.66		98.43635

				178.68		98.43635

				178.7		98.43635

				178.73		98.43247

				178.75		98.43247

				178.77		98.43247

				178.79		98.42859

				178.81		98.42471

				178.83		98.42471

				178.85		98.42471

				178.87		98.42471

				178.89		98.42083

				178.91		98.41695

				178.94		98.41307

				178.96		98.41307

				178.98		98.40919

				179		98.40919

				179.02		98.40531

				179.04		98.40531

				179.06		98.39755

				179.08		98.39367

				179.1		98.38979

				179.12		98.38979

				179.15		98.38591

				179.17		98.38591

				179.19		98.37815

				179.21		98.37427

				179.23		98.38203

				179.25		98.37427

				179.27		98.37427

				179.29		98.37427

				179.31		98.37039

				179.33		98.35875

				179.35		98.36263

				179.38		98.35487

				179.4		98.35487

				179.42		98.34323

				179.44		98.35099

				179.46		98.34323

				179.48		98.33159

				179.5		98.33159

				179.52		98.32771

				179.54		98.32771

				179.56		98.32382

				179.59		98.31606

				179.61		98.31218

				179.63		98.3083

				179.65		98.30442

				179.67		98.30442

				179.69		98.30054

				179.71		98.30442

				179.73		98.29666

				179.75		98.29666

				179.77		98.29666

				179.79		98.29278

				179.82		98.29278

				179.84		98.2889

				179.86		98.28114

				179.88		98.28114

				179.9		98.27726

				179.92		98.27726

				179.94		98.27338

				179.96		98.2695

				179.98		98.26562

				180		98.26562

				180.03		98.25786

				180.05		98.25786

				180.07		98.2501

				180.09		98.2501

				180.11		98.24622

				180.13		98.24622

				180.15		98.24234

				180.17		98.24234

				180.19		98.23846

				180.21		98.24234

				180.24		98.24234

				180.26		98.23846

				180.28		98.24234

				180.3		98.23846

				180.32		98.23846

				180.34		98.23846

				180.36		98.23846

				180.38		98.23846

				180.4		98.2307

				180.42		98.2307

				180.44		98.22682

				180.47		98.22682

				180.49		98.22294

				180.51		98.21906

				180.53		98.21518

				180.55		98.2113

				180.57		98.20742

				180.59		98.20742

				180.61		98.19966

				180.63		98.20354

				180.65		98.19966

				180.68		98.19578

				180.7		98.18802

				180.72		98.18414

				180.74		98.18026

				180.76		98.18026

				180.78		98.17638

				180.8		98.17638

				180.82		98.16862

				180.84		98.16474

				180.86		98.16474

				180.89		98.16086

				180.91		98.15698

				180.93		98.14922

				180.95		98.14922

				180.97		98.14534

				180.99		98.14146

				181.01		98.14146

				181.03		98.1337

				181.05		98.14146

				181.07		98.1337

				181.1		98.12982

				181.12		98.12594

				181.14		98.12594

				181.16		98.12206

				181.18		98.12206

				181.2		98.11818

				181.22		98.12206

				181.24		98.11818

				181.26		98.11042

				181.28		98.11042

				181.31		98.11042

				181.33		98.09878

				181.35		98.0949

				181.37		98.09878

				181.39		98.08326

				181.41		98.08326

				181.43		98.08326

				181.45		98.08326

				181.47		98.06774

				181.49		98.06774

				181.51		98.06774

				181.54		98.05998

				181.56		98.0561

				181.58		98.06386

				181.6		98.05998

				181.62		98.06386

				181.64		98.06386

				181.66		98.05998

				181.68		98.0561

				181.7		98.0561

				181.72		98.05998

				181.75		98.05222

				181.77		98.04834

				181.79		98.05222

				181.81		98.05222

				181.83		98.04834

				181.85		98.04446

				181.87		98.04834

				181.89		98.03282

				181.91		98.02894

				181.93		98.02894

				181.95		98.02118

				181.98		98.01342

				182		98.01342

				182.02		98.01342

				182.04		98.00178

				182.06		97.9979

				182.08		97.99402

				182.1		97.99402

				182.12		97.99014

				182.14		97.98626

				182.16		97.97462

				182.19		97.98626

				182.21		97.9785

				182.23		97.97462

				182.25		97.97462

				182.27		97.97462

				182.29		97.96298

				182.31		97.96298

				182.33		97.9591

				182.35		97.95522

				182.37		97.95522

				182.4		97.94746

				182.42		97.94746

				182.44		97.9397

				182.46		97.93194

				182.48		97.93194

				182.5		97.93194

				182.52		97.92418

				182.54		97.92418

				182.56		97.9203

				182.58		97.90866

				182.61		97.91254

				182.63		97.90866

				182.65		97.9009

				182.67		97.9009

				182.69		97.89314

				182.71		97.89702

				182.73		97.89314

				182.75		97.88926

				182.77		97.8815

				182.79		97.8815

				182.82		97.87762

				182.84		97.87762

				182.86		97.87374

				182.88		97.86598

				182.9		97.86598

				182.92		97.86598

				182.94		97.85434

				182.96		97.85434

				182.98		97.85434

				183		97.84658

				183.02		97.8427

				183.05		97.8427

				183.07		97.83882

				183.09		97.83494

				183.11		97.82718

				183.13		97.82718

				183.15		97.82718

				183.17		97.82718

				183.19		97.8233

				183.21		97.81942

				183.23		97.81554

				183.26		97.81166

				183.28		97.80778

				183.3		97.80778

				183.32		97.80778

				183.34		97.79614

				183.36		97.80002

				183.38		97.79614

				183.4		97.78838

				183.42		97.78838

				183.44		97.7845

				183.47		97.7845

				183.49		97.77286

				183.51		97.77286

				183.53		97.77286

				183.55		97.76122

				183.57		97.76122

				183.59		97.75734

				183.61		97.75346

				183.63		97.74958

				183.65		97.74958

				183.67		97.7457

				183.7		97.74182

				183.72		97.74182

				183.74		97.7457

				183.76		97.73406

				183.78		97.73018

				183.8		97.73406

				183.82		97.73018

				183.84		97.72242

				183.86		97.72242

				183.88		97.71854

				183.91		97.71854

				183.93		97.71466

				183.95		97.71078

				183.97		97.7069

				183.99		97.70302

				184.01		97.70302

				184.03		97.69914

				184.05		97.6875

				184.07		97.69526

				184.09		97.6875

				184.11		97.67974

				184.14		97.67586

				184.16		97.67974

				184.18		97.67198

				184.2		97.6681

				184.22		97.66422

				184.24		97.66034

				184.26		97.6681

				184.28		97.66422

				184.3		97.66034

				184.32		97.65646

				184.35		97.6487

				184.37		97.6487

				184.39		97.64482

				184.41		97.64094

				184.43		97.64482

				184.45		97.6293

				184.47		97.6293

				184.49		97.63318

				184.51		97.62542

				184.53		97.61766

				184.55		97.6099

				184.58		97.60602

				184.6		97.60602

				184.62		97.60214

				184.64		97.60602

				184.66		97.60214

				184.68		97.60214

				184.7		97.59826

				184.72		97.60214

				184.74		97.59438

				184.76		97.5905

				184.79		97.5905

				184.81		97.5905

				184.83		97.58274

				184.85		97.57886

				184.87		97.57886

				184.89		97.5711

				184.91		97.56722

				184.93		97.56334

				184.95		97.55558

				184.97		97.55558

				184.99		97.54782

				185.02		97.54394

				185.04		97.54006

				185.06		97.5323

				185.08		97.52842

				185.1		97.52842

				185.12		97.52454

				185.14		97.51678

				185.16		97.50902

				185.18		97.50902

				185.2		97.50126

				185.22		97.50126

				185.25		97.49738

				185.27		97.49738

				185.29		97.4935

				185.31		97.48574

				185.33		97.48962

				185.35		97.48186

				185.37		97.47798

				185.39		97.47798

				185.41		97.4741

				185.43		97.4741

				185.46		97.46634

				185.48		97.47022

				185.5		97.45858

				185.52		97.4547

				185.54		97.45082

				185.56		97.44694

				185.58		97.44306

				185.6		97.43918

				185.62		97.43918

				185.64		97.4353

				185.66		97.42754

				185.69		97.43142

				185.71		97.42366

				185.73		97.41978

				185.75		97.4159

				185.77		97.41978

				185.79		97.40814

				185.81		97.40814

				185.83		97.40038

				185.85		97.40426

				185.87		97.3965

				185.9		97.38874

				185.92		97.38486

				185.94		97.38486

				185.96		97.36934

				185.98		97.36934

				186		97.36546

				186.02		97.3577

				186.04		97.35382

				186.06		97.35382

				186.08		97.34994

				186.1		97.34994

				186.13		97.34218

				186.15		97.3383

				186.17		97.33054

				186.19		97.32666

				186.21		97.32278

				186.23		97.32666

				186.25		97.32278

				186.27		97.32666

				186.29		97.3189

				186.31		97.3189

				186.34		97.30726

				186.36		97.30726

				186.38		97.2995

				186.4		97.29562

				186.42		97.29562

				186.44		97.29174

				186.46		97.28786

				186.48		97.2801

				186.5		97.27622

				186.52		97.26846

				186.55		97.26458

				186.57		97.2607

				186.59		97.26458

				186.61		97.2607

				186.63		97.25682

				186.65		97.25682

				186.67		97.25294

				186.69		97.25294

				186.71		97.24906

				186.73		97.2413

				186.75		97.23742

				186.78		97.23354

				186.8		97.22578

				186.82		97.2219

				186.84		97.21802

				186.86		97.21802

				186.88		97.21025

				186.9		97.20637

				186.92		97.19861

				186.94		97.19861

				186.96		97.19473

				186.98		97.19085

				187.01		97.19085

				187.03		97.18697

				187.05		97.18309

				187.07		97.17921

				187.09		97.17145

				187.11		97.15981

				187.13		97.15981

				187.15		97.15593

				187.17		97.14817

				187.19		97.14817

				187.22		97.14429

				187.24		97.14041

				187.26		97.14041

				187.28		97.12489

				187.3		97.12489

				187.32		97.11325

				187.34		97.12101

				187.36		97.11325

				187.38		97.11325

				187.4		97.10549

				187.42		97.10161

				187.45		97.09773

				187.47		97.08997

				187.49		97.08997

				187.51		97.09385

				187.53		97.07833

				187.55		97.08609

				187.57		97.07445

				187.59		97.07057

				187.61		97.06281

				187.63		97.06281

				187.66		97.05893

				187.68		97.05505

				187.7		97.05117

				187.72		97.03953

				187.74		97.03953

				187.76		97.03953

				187.78		97.02401

				187.8		97.02789

				187.82		97.02789

				187.84		97.02401

				187.86		97.01237

				187.89		97.00849

				187.91		97.01237

				187.93		97.00849

				187.95		97.01237

				187.97		97.00849

				187.99		97.00461

				188.01		97.00849

				188.03		97.00461

				188.05		96.99685

				188.07		96.99685

				188.1		96.99685

				188.12		96.99297

				188.14		96.98521

				188.16		96.97745

				188.18		96.97745

				188.2		96.96581

				188.22		96.96193

				188.24		96.95805

				188.26		96.95805

				188.28		96.94641

				188.31		96.94641

				188.33		96.94253

				188.35		96.93865

				188.37		96.92701

				188.39		96.93089

				188.41		96.91925

				188.43		96.91537

				188.45		96.91149

				188.47		96.90761

				188.49		96.90373

				188.51		96.90373

				188.54		96.89597

				188.56		96.89597

				188.58		96.88821

				188.6		96.89209

				188.62		96.88433

				188.64		96.87657

				188.66		96.88045

				188.68		96.87269

				188.7		96.86881

				188.72		96.85717

				188.75		96.86105

				188.77		96.85329

				188.79		96.84553

				188.81		96.83777

				188.83		96.83777

				188.85		96.83001

				188.87		96.83389

				188.89		96.82613

				188.91		96.82225

				188.93		96.81837

				188.95		96.81061

				188.98		96.80673

				189		96.80673

				189.02		96.79509

				189.04		96.78345

				189.06		96.78345

				189.08		96.77569

				189.1		96.76793

				189.12		96.76405

				189.14		96.76017

				189.16		96.75629

				189.19		96.74853

				189.21		96.75241

				189.23		96.74077

				189.25		96.73689

				189.27		96.74077

				189.29		96.72913

				189.31		96.72525

				189.33		96.71749

				189.35		96.71749

				189.37		96.70973

				189.4		96.70973

				189.42		96.70585

				189.44		96.70973

				189.46		96.69421

				189.48		96.70197

				189.5		96.68645

				189.52		96.69033

				189.54		96.68257

				189.56		96.68257

				189.58		96.66317

				189.6		96.66705

				189.63		96.65541

				189.65		96.64765

				189.67		96.64377

				189.69		96.64377

				189.71		96.63601

				189.73		96.63601

				189.75		96.62825

				189.77		96.63213

				189.79		96.62437

				189.81		96.62049

				189.84		96.62437

				189.86		96.60885

				189.88		96.60885

				189.9		96.60497

				189.92		96.59721

				189.94		96.58945

				189.96		96.58557

				189.98		96.58169

				190		96.57005

				190.02		96.56229

				190.05		96.56229

				190.07		96.55841

				190.09		96.55065

				190.11		96.54677

				190.13		96.54289

				190.15		96.53513

				190.17		96.53125

				190.19		96.53125

				190.21		96.53125

				190.23		96.52737

				190.25		96.51573

				190.28		96.51961

				190.3		96.50797

				190.32		96.50797

				190.34		96.50021

				190.36		96.50021

				190.38		96.48857

				190.4		96.48857

				190.42		96.48081

				190.44		96.48469

				190.46		96.47693

				190.49		96.47693

				190.51		96.46917

				190.53		96.46141

				190.55		96.45753

				190.57		96.45753

				190.59		96.44201

				190.61		96.43813

				190.63		96.43037

				190.65		96.41873

				190.67		96.40709

				190.7		96.40321

				190.72		96.40709

				190.74		96.39545

				190.76		96.39157

				190.78		96.39157

				190.8		96.38769

				190.82		96.38381

				190.84		96.38769

				190.86		96.39933

				190.88		96.39157

				190.91		96.38381

				190.93		96.38769

				190.95		96.37605

				190.97		96.37605

				190.99		96.37993

				191.01		96.36441

				191.03		96.35277

				191.05		96.33725

				191.07		96.34113

				191.09		96.32561

				191.11		96.32561

				191.14		96.32561

				191.16		96.31397

				191.18		96.30233

				191.2		96.30233

				191.22		96.30233

				191.24		96.29457

				191.26		96.28681

				191.28		96.29457

				191.3		96.27517

				191.32		96.27129

				191.35		96.27129

				191.37		96.27129

				191.39		96.26353

				191.41		96.25965

				191.43		96.26353

				191.45		96.24801

				191.47		96.24801

				191.49		96.24025

				191.51		96.23249

				191.53		96.23249

				191.56		96.22085

				191.58		96.22473

				191.6		96.21309

				191.62		96.20145

				191.64		96.20145

				191.66		96.18981

				191.68		96.18205

				191.7		96.17817

				191.72		96.17041

				191.74		96.15877

				191.76		96.15101

				191.79		96.15877

				191.81		96.14713

				191.83		96.15101

				191.85		96.14325

				191.87		96.14713

				191.89		96.13937

				191.91		96.13937

				191.93		96.13937

				191.95		96.13161

				191.97		96.12385

				192		96.12385

				192.02		96.11221

				192.04		96.10833

				192.06		96.10057

				192.08		96.10057

				192.1		96.08504

				192.12		96.07728

				192.14		96.0734

				192.16		96.06176

				192.18		96.06176

				192.2		96.05012

				192.23		96.054

				192.25		96.04236

				192.27		96.03848

				192.29		96.04236

				192.31		96.0346

				192.33		96.0346

				192.35		96.0346

				192.37		96.02684

				192.39		96.02684

				192.41		96.01908

				192.43		96.02684

				192.46		96.01908

				192.48		96.00744

				192.5		96.01132

				192.52		95.99968

				192.54		95.99192

				192.56		95.98416

				192.58		95.98416

				192.6		95.98028

				192.62		95.96476

				192.64		95.96088

				192.67		95.96088

				192.69		95.94536

				192.71		95.94924

				192.73		95.94536

				192.75		95.94536

				192.77		95.92596

				192.79		95.92596

				192.81		95.92596

				192.83		95.9182

				192.85		95.91044

				192.87		95.91044

				192.9		95.8988

				192.92		95.8988

				192.94		95.89104

				192.96		95.89104

				192.98		95.88328

				193		95.88716

				193.02		95.87164

				193.04		95.86776

				193.06		95.86388

				193.08		95.86388

				193.1		95.84448

				193.13		95.84448

				193.15		95.8406

				193.17		95.83284

				193.19		95.81732

				193.21		95.8212

				193.23		95.81344

				193.25		95.80568

				193.27		95.80568

				193.29		95.80568

				193.31		95.79404

				193.33		95.79404

				193.36		95.79404

				193.38		95.7824

				193.4		95.77852

				193.42		95.77852

				193.44		95.77852

				193.46		95.75912

				193.48		95.75524

				193.5		95.75524

				193.52		95.73972

				193.54		95.72808

				193.56		95.73196

				193.59		95.72808

				193.61		95.70868

				193.63		95.70092

				193.65		95.7048

				193.67		95.69316

				193.69		95.6854

				193.71		95.6854

				193.73		95.6854

				193.75		95.67764

				193.77		95.67376

				193.79		95.67376

				193.82		95.666

				193.84		95.66212

				193.86		95.666

				193.88		95.66212

				193.9		95.65048

				193.92		95.6466

				193.94		95.64272

				193.96		95.63496

				193.98		95.63108

				194		95.63108

				194.02		95.61944

				194.05		95.60392

				194.07		95.60392

				194.09		95.59228

				194.11		95.5884

				194.13		95.57676

				194.15		95.57288

				194.17		95.56124

				194.19		95.5496

				194.21		95.55736

				194.23		95.55736

				194.26		95.5496

				194.28		95.5496

				194.3		95.55348

				194.32		95.54184

				194.34		95.53408

				194.36		95.53796

				194.38		95.52632

				194.4		95.51856

				194.42		95.50692

				194.44		95.5108

				194.46		95.50304

				194.49		95.50304

				194.51		95.48752

				194.53		95.472

				194.55		95.46424

				194.57		95.45648

				194.59		95.44484

				194.61		95.44484

				194.63		95.42932

				194.65		95.42544

				194.67		95.42932

				194.69		95.42156

				194.72		95.42156

				194.74		95.41768

				194.76		95.40604

				194.78		95.40216

				194.8		95.3944

				194.82		95.3944

				194.84		95.38664

				194.86		95.38276

				194.88		95.38276

				194.9		95.36724

				194.92		95.375

				194.95		95.3556

				194.97		95.3556

				194.99		95.34008

				195.01		95.3362

				195.03		95.32068

				195.05		95.3168

				195.07		95.2974

				195.09		95.30516

				195.11		95.278

				195.13		95.28188

				195.15		95.27412

				195.18		95.27024

				195.2		95.27412

				195.22		95.278

				195.24		95.27412

				195.26		95.27412

				195.28		95.26636

				195.3		95.26248

				195.32		95.26248

				195.34		95.24696

				195.36		95.24696

				195.39		95.23532

				195.41		95.22756

				195.43		95.22756

				195.45		95.2198

				195.47		95.20428

				195.49		95.2004

				195.51		95.18876

				195.53		95.181

				195.55		95.17712

				195.57		95.16936

				195.59		95.1616

				195.62		95.14608

				195.64		95.1422

				195.66		95.13832

				195.68		95.13056

				195.7		95.11892

				195.72		95.11892

				195.74		95.11116

				195.76		95.11504

				195.78		95.1034

				195.8		95.10728

				195.83		95.09564

				195.85		95.09952

				195.87		95.08788

				195.89		95.09176

				195.91		95.07236

				195.93		95.07236

				195.95		95.0646

				195.97		95.05684

				195.99		95.04908

				196.01		95.04908

				196.03		95.02968

				196.06		95.01804

				196.08		95.02192

				196.1		95.0064

				196.12		94.99864

				196.14		94.98312

				196.16		94.98312

				196.18		94.97535

				196.2		94.97535

				196.22		94.95983

				196.24		94.96371

				196.26		94.95983

				196.29		94.96759

				196.31		94.95595

				196.33		94.95595

				196.35		94.95207

				196.37		94.95983

				196.39		94.94043

				196.41		94.93655

				196.43		94.93267

				196.45		94.91715

				196.47		94.90939

				196.5		94.90163

				196.52		94.88611

				196.54		94.87835

				196.56		94.87059

				196.58		94.86283

				196.6		94.86671

				196.62		94.85119

				196.64		94.85507

				196.66		94.84731

				196.68		94.83955

				196.7		94.82791

				196.73		94.82403

				196.75		94.81239

				196.77		94.80851

				196.79		94.80851

				196.81		94.80851

				196.83		94.80075

				196.85		94.79299

				196.87		94.79299

				196.89		94.78911

				196.91		94.78523

				196.93		94.77359

				196.96		94.76583

				196.98		94.75419

				197		94.75807

				197.02		94.74643

				197.04		94.73091

				197.06		94.72315

				197.08		94.70763

				197.1		94.69599

				197.12		94.69211

				197.14		94.68823

				197.17		94.68047

				197.19		94.68047

				197.21		94.66883

				197.23		94.68047

				197.25		94.67271

				197.27		94.67659

				197.29		94.65719

				197.31		94.66495

				197.33		94.64943

				197.35		94.65331

				197.37		94.63391

				197.4		94.62227

				197.42		94.61451

				197.44		94.61451

				197.46		94.59511

				197.48		94.59123

				197.5		94.57959

				197.52		94.57959

				197.54		94.57183

				197.56		94.56795

				197.58		94.56019

				197.6		94.55243

				197.63		94.54855

				197.65		94.54467

				197.67		94.54467

				197.69		94.53691

				197.71		94.52527

				197.73		94.52139

				197.75		94.51751

				197.77		94.50587

				197.79		94.50587

				197.81		94.49035

				197.84		94.48259

				197.86		94.47483

				197.88		94.46319

				197.9		94.45543

				197.92		94.43603

				197.94		94.42827

				197.96		94.41663

				197.98		94.41275

				198		94.40111

				198.02		94.40111

				198.05		94.38559

				198.07		94.39335

				198.09		94.39723

				198.11		94.39335

				198.13		94.38171

				198.15		94.37783

				198.17		94.37783

				198.19		94.37007

				198.21		94.36619

				198.23		94.34291

				198.25		94.35067

				198.28		94.34291

				198.3		94.33903

				198.32		94.33127

				198.34		94.31963

				198.36		94.31575

				198.38		94.31187

				198.4		94.28859

				198.42		94.28083

				198.44		94.27695

				198.46		94.26143

				198.49		94.26143

				198.51		94.24979

				198.53		94.24203

				198.55		94.23039

				198.57		94.23427

				198.59		94.21487

				198.61		94.20711

				198.63		94.19547

				198.65		94.19547

				198.67		94.19547

				198.69		94.18771

				198.72		94.17995

				198.74		94.18383

				198.76		94.17607

				198.78		94.17219

				198.8		94.16055

				198.82		94.13727

				198.84		94.12951

				198.86		94.11787

				198.88		94.11011

				198.9		94.10235

				198.92		94.10623

				198.95		94.09459

				198.97		94.09071

				198.99		94.08683

				199.01		94.09071

				199.03		94.07907

				199.05		94.07519

				199.07		94.05579

				199.09		94.05967

				199.11		94.05579

				199.13		94.04027

				199.15		94.03251

				199.18		94.02475

				199.2		94.02087

				199.22		94.01699

				199.24		94.00147

				199.26		93.98595

				199.28		93.99371

				199.3		93.98983

				199.32		93.98595

				199.34		93.97431

				199.36		93.96267

				199.39		93.95491

				199.41		93.95103

				199.43		93.93939

				199.45		93.92387

				199.47		93.91223

				199.49		93.91223

				199.51		93.91611

				199.53		93.90447

				199.55		93.90059

				199.57		93.89671

				199.59		93.88895

				199.62		93.88507

				199.64		93.87343

				199.66		93.8579

				199.68		93.85402

				199.7		93.84626

				199.72		93.84626

				199.74		93.82298

				199.76		93.82298

				199.78		93.81134

				199.8		93.81134

				199.82		93.80746

				199.85		93.77642

				199.87		93.79582

				199.89		93.77642

				199.91		93.76478

				199.93		93.73762

				199.95		93.73762

				199.97		93.72598

				199.99		93.70658

				200.01		93.7027

				200.03		93.71434

				200.05		93.70658

				200.08		93.68718

				200.1		93.70658

				200.12		93.71046

				200.14		93.69882

				200.16		93.6833

				200.18		93.69106

				200.2		93.66778

				200.22		93.65614

				200.24		93.6445

				200.26		93.6445

				200.29		93.63286

				200.31		93.61734

				200.33		93.61346

				200.35		93.60958

				200.37		93.57854

				200.39		93.57078

				200.41		93.5669

				200.43		93.56302

				200.45		93.54362

				200.47		93.55914

				200.49		93.55138

				200.52		93.53198

				200.54		93.53974

				200.56		93.53586

				200.58		93.53198

				200.6		93.50482

				200.62		93.5281

				200.64		93.49318

				200.66		93.49318

				200.68		93.46602

				200.7		93.48542

				200.73		93.45438

				200.75		93.4505

				200.77		93.4311

				200.79		93.44274

				200.81		93.42334

				200.83		93.40782

				200.85		93.39618

				200.87		93.38454

				200.89		93.3729

				200.91		93.34962

				200.93		93.3729

				200.96		93.3535

				200.98		93.36126

				201		93.34574

				201.02		93.36126

				201.04		93.33022

				201.06		93.33798

				201.08		93.32634

				201.1		93.3341

				201.12		93.31858

				201.14		93.32246

				201.17		93.31858

				201.19		93.30694

				201.21		93.29142

				201.23		93.28366

				201.25		93.2759

				201.27		93.26038

				201.29		93.2565

				201.31		93.24874

				201.33		93.24486

				201.35		93.22934

				201.37		93.23322

				201.4		93.22546

				201.42		93.22546

				201.44		93.21382

				201.46		93.22158

				201.48		93.20994

				201.5		93.20218

				201.52		93.1789

				201.54		93.1789

				201.56		93.1595

				201.58		93.1401

				201.61		93.1401

				201.63		93.13622

				201.65		93.12458

				201.67		93.10906

				201.69		93.10906

				201.71		93.1013

				201.73		93.08966

				201.75		93.07802

				201.77		93.07802

				201.79		93.06638

				201.81		93.05862

				201.84		93.03922

				201.86		93.02758

				201.88		93.01594

				201.9		93.01206

				201.92		92.98878

				201.94		92.9849

				201.96		92.98102

				201.98		92.97326

				202		92.96162

				202.02		92.96938

				202.05		92.96162

				202.07		92.94998

				202.09		92.95386

				202.11		92.93834

				202.13		92.92282

				202.15		92.91506

				202.17		92.9073

				202.19		92.89178

				202.21		92.89178

				202.23		92.88402

				202.26		92.89178

				202.28		92.88014

				202.3		92.86074

				202.32		92.8491

				202.34		92.84522

				202.36		92.82194

				202.38		92.82194

				202.4		92.82194

				202.42		92.8103

				202.44		92.8103

				202.46		92.80254

				202.49		92.79478

				202.51		92.7715

				202.53		92.77926

				202.55		92.75598

				202.57		92.75598

				202.59		92.74433

				202.61		92.75598

				202.63		92.72105

				202.65		92.72105

				202.67		92.70941

				202.69		92.70941

				202.72		92.69389

				202.74		92.70553

				202.76		92.67837

				202.78		92.67449

				202.8		92.66285

				202.82		92.65897

				202.84		92.63181

				202.86		92.63569

				202.88		92.62405

				202.9		92.62017

				202.93		92.61241

				202.95		92.61629

				202.97		92.61241

				202.99		92.60077

				203.01		92.59689

				203.03		92.58913

				203.05		92.58137

				203.07		92.56585

				203.09		92.56585

				203.11		92.55421

				203.14		92.52705

				203.16		92.51541

				203.18		92.51153

				203.2		92.49213

				203.22		92.48825

				203.24		92.48825

				203.26		92.47273

				203.28		92.45721

				203.3		92.44945

				203.32		92.44169

				203.34		92.42617

				203.37		92.41453

				203.39		92.43005

				203.41		92.42617

				203.43		92.40289

				203.45		92.40289

				203.47		92.41065

				203.49		92.38737

				203.51		92.37573

				203.53		92.38737

				203.55		92.37573

				203.58		92.35245

				203.6		92.35245

				203.62		92.33305

				203.64		92.31753

				203.66		92.30977

				203.68		92.30977

				203.7		92.29037

				203.72		92.27485

				203.74		92.26321

				203.76		92.25933

				203.78		92.23605

				203.81		92.23605

				203.83		92.24769

				203.85		92.22053

				203.87		92.21277

				203.89		92.20501

				203.91		92.19725

				203.93		92.17397

				203.95		92.18561

				203.97		92.17009

				203.99		92.16233

				204.02		92.15069

				204.04		92.16233

				204.06		92.12741

				204.08		92.11577

				204.1		92.11189

				204.12		92.10025

				204.14		92.08473

				204.16		92.08861

				204.18		92.07697

				204.2		92.04205

				204.23		92.04981

				204.25		92.04593

				204.27		92.03041

				204.29		92.01877

				204.31		92.03429

				204.33		92.01101

				204.35		92.00325

				204.37		91.99937

				204.39		92.00713

				204.41		91.99549

				204.43		91.98773

				204.46		91.97997

				204.48		91.96833

				204.5		91.94117

				204.52		91.93341

				204.54		91.93341

				204.56		91.90625

				204.58		91.89461

				204.6		91.89461

				204.62		91.88685

				204.64		91.84417

				204.67		91.85581

				204.69		91.84417

				204.71		91.82477

				204.73		91.80149

				204.75		91.82089

				204.77		91.79761

				204.79		91.78209

				204.81		91.78209

				204.83		91.78597

				204.85		91.76657

				204.88		91.76657

				204.9		91.75881

				204.92		91.74329

				204.94		91.73941

				204.96		91.72777

				204.98		91.72389

				205		91.70837

				205.02		91.71225

				205.04		91.69285

				205.06		91.68121

				205.08		91.66569

				205.11		91.66181

				205.13		91.63853

				205.15		91.62688

				205.17		91.623

				205.19		91.61912

				205.21		91.59972

				205.23		91.61136

				205.25		91.6036

				205.27		91.58808

				205.29		91.56868

				205.31		91.58808

				205.34		91.5648

				205.36		91.5454

				205.38		91.56092

				205.4		91.54152

				205.42		91.51824

				205.44		91.51824

				205.46		91.526

				205.48		91.49496

				205.5		91.49108

				205.52		91.4872

				205.55		91.4678

				205.57		91.44064

				205.59		91.4484

				205.61		91.43676

				205.63		91.42124

				205.65		91.4096

				205.67		91.41736

				205.69		91.40184

				205.71		91.38244

				205.73		91.39408

				205.75		91.37856

				205.78		91.36304

				205.8		91.3514

				205.82		91.3708

				205.84		91.33588

				205.86		91.33976

				205.88		91.33588

				205.9		91.332

				205.92		91.30096

				205.94		91.29708

				205.96		91.28156

				205.99		91.2544

				206.01		91.24276

				206.03		91.23888

				206.05		91.22724

				206.07		91.21172

				206.09		91.2156

				206.11		91.1962

				206.13		91.18068

				206.15		91.1768

				206.17		91.1768

				206.19		91.14964

				206.22		91.1574

				206.24		91.16128

				206.26		91.138

				206.28		91.12636

				206.3		91.138

				206.32		91.12248

				206.34		91.09144

				206.36		91.09144

				206.38		91.08368

				206.4		91.05264

				206.43		91.03712

				206.45		91.05264

				206.47		91.03712

				206.49		91.01384

				206.51		91.01384

				206.53		91.0022

				206.55		90.96728

				206.57		90.95952

				206.59		90.9634

				206.61		90.95564

				206.64		90.94012

				206.66		90.94788

				206.68		90.93624

				206.7		90.92072

				206.72		90.90908

				206.74		90.90908

				206.76		90.8858

				206.78		90.88968

				206.8		90.90132

				206.82		90.8858

				206.84		90.8664

				206.87		90.88192

				206.89		90.85864

				206.91		90.8276

				206.93		90.81208

				206.95		90.81208

				206.97		90.77328

				206.99		90.76552

				207.01		90.76164

				207.03		90.76164

				207.05		90.74224

				207.07		90.7306

				207.1		90.72284

				207.12		90.69568

				207.14		90.68016

				207.16		90.67628

				207.18		90.67628

				207.2		90.65688

				207.22		90.65688

				207.24		90.66076

				207.26		90.64136

				207.28		90.63748

				207.3		90.63748

				207.33		90.6336

				207.35		90.60256

				207.37		90.60644

				207.39		90.59092

				207.41		90.56376

				207.43		90.54048

				207.45		90.54436

				207.47		90.5172

				207.49		90.50167

				207.51		90.50167

				207.54		90.49779

				207.56		90.46675

				207.58		90.45511

				207.6		90.45123

				207.62		90.42795

				207.64		90.40467

				207.66		90.41243

				207.68		90.40855

				207.7		90.38915

				207.72		90.40079

				207.74		90.38915

				207.77		90.36975

				207.79		90.35423

				207.81		90.35035

				207.83		90.33871

				207.85		90.32319

				207.87		90.32319

				207.89		90.31931

				207.91		90.30767

				207.93		90.28439

				207.95		90.28051

				207.97		90.26111

				208		90.23395

				208.02		90.22619

				208.04		90.21843

				208.06		90.19515

				208.08		90.19127

				208.1		90.18739

				208.12		90.16411

				208.14		90.15635

				208.16		90.15635

				208.18		90.14083

				208.2		90.12919

				208.23		90.13307

				208.25		90.11367

				208.27		90.10591

				208.29		90.09039

				208.31		90.09427

				208.33		90.06323

				208.35		90.05935

				208.37		90.05159

				208.39		90.05159

				208.41		90.02055

				208.43		90.02443

				208.46		90.01667

				208.48		90.00115

				208.5		89.97399

				208.52		89.97011

				208.54		89.96235

				208.56		89.93907

				208.58		89.91967

				208.6		89.91967

				208.62		89.91579

				208.64		89.88863

				208.66		89.90027

				208.69		89.90027

				208.71		89.87699

				208.73		89.85759

				208.75		89.86923

				208.77		89.83431

				208.79		89.81879

				208.81		89.82655

				208.83		89.81491

				208.85		89.78775

				208.87		89.78775

				208.89		89.77999

				208.92		89.75283

				208.94		89.73731

				208.96		89.73343

				208.98		89.71791

				209		89.68687

				209.02		89.68687

				209.04		89.68687

				209.06		89.66747

				209.08		89.64419

				209.1		89.65583

				209.12		89.63643

				209.15		89.61703

				209.17		89.61315

				209.19		89.60927

				209.21		89.58211

				209.23		89.57823

				209.25		89.56659

				209.27		89.55495

				209.29		89.53943

				209.31		89.54331

				209.33		89.52391

				209.35		89.50839

				209.38		89.51615

				209.4		89.49675

				209.42		89.47735

				209.44		89.46571

				209.46		89.48123

				209.48		89.44243

				209.5		89.43855

				209.52		89.42691

				209.54		89.41527

				209.56		89.3881

				209.58		89.3881

				209.61		89.37646

				209.63		89.35706

				209.65		89.34154

				209.67		89.3299

				209.69		89.32602

				209.71		89.29498

				209.73		89.29498

				209.75		89.2911

				209.77		89.27558

				209.79		89.25618

				209.81		89.2717

				209.84		89.24454

				209.86		89.2329

				209.88		89.22514

				209.9		89.20962

				209.92		89.19022

				209.94		89.19022

				209.96		89.19022

				209.98		89.16306

				210		89.16306

				210.02		89.14754

				210.04		89.12814

				210.07		89.10098

				210.09		89.08934

				210.11		89.07382

				210.13		89.06606

				210.15		89.05054

				210.17		89.04278

				210.19		89.0389

				210.21		89.0195

				210.23		89.00398

				210.25		89.0001

				210.28		88.98846

				210.3		88.98458

				210.32		88.9807

				210.34		88.96518

				210.36		88.94966

				210.38		88.95354

				210.4		88.9225

				210.42		88.91474

				210.44		88.9031

				210.46		88.89146

				210.48		88.87594

				210.51		88.8643

				210.53		88.85266

				210.55		88.83326

				210.57		88.82938

				210.59		88.79446

				210.61		88.80222

				210.63		88.76342

				210.65		88.76342

				210.67		88.74402

				210.69		88.7479

				210.71		88.71686

				210.74		88.74014

				210.76		88.7285

				210.78		88.72074

				210.8		88.69358

				210.82		88.70522

				210.84		88.6703

				210.86		88.64702

				210.88		88.64702

				210.9		88.65478

				210.92		88.62374

				210.94		88.6121

				210.97		88.60434

				210.99		88.58882

				211.01		88.5539

				211.03		88.54614

				211.05		88.54226

				211.07		88.52286

				211.09		88.49958

				211.11		88.49958

				211.13		88.48406

				211.15		88.4569

				211.17		88.44914

				211.2		88.44138

				211.22		88.4181

				211.24		88.4181

				211.26		88.41034

				211.28		88.40646

				211.3		88.37542

				211.32		88.38318

				211.34		88.37154

				211.36		88.35214

				211.38		88.33662

				211.4		88.3405

				211.43		88.31722

				211.45		88.29782

				211.47		88.28229

				211.49		88.28229

				211.51		88.26677

				211.53		88.25901

				211.55		88.22409

				211.57		88.21633

				211.59		88.18529

				211.61		88.17365

				211.63		88.15037

				211.66		88.15813

				211.68		88.15037

				211.7		88.13873

				211.72		88.11933

				211.74		88.12321

				211.76		88.10381

				211.78		88.08829

				211.8		88.08441

				211.82		88.09217

				211.84		88.06113

				211.86		88.04949

				211.89		88.04561

				211.91		88.01069

				211.93		87.98353

				211.95		87.97577

				211.97		87.97189

				211.99		87.94085

				212.01		87.94473

				212.03		87.93309

				212.05		87.91369

				212.07		87.89041

				212.09		87.88265

				212.12		87.87101

				212.14		87.83997

				212.16		87.84385

				212.18		87.83609

				212.2		87.83997

				212.22		87.80893

				212.24		87.81669

				212.26		87.81669

				212.28		87.79341

				212.3		87.75461

				212.32		87.76625

				212.35		87.75073

				212.37		87.71581

				212.39		87.71581

				212.41		87.71193

				212.43		87.67701

				212.45		87.67313

				212.47		87.67313

				212.49		87.63821

				212.51		87.63821

				212.53		87.63045

				212.55		87.61493

				212.58		87.58777

				212.6		87.58389

				212.62		87.57225

				212.64		87.54897

				212.66		87.53733

				212.68		87.54897

				212.7		87.54121

				212.72		87.51405

				212.74		87.52569

				212.76		87.50629

				212.78		87.47525

				212.81		87.46749

				212.83		87.45585

				212.85		87.42869

				212.87		87.41317

				212.89		87.39765

				212.91		87.37437

				212.93		87.36661

				212.95		87.35109

				212.97		87.33557

				212.99		87.32393

				213.01		87.30453

				213.04		87.29677

				213.06		87.26573

				213.08		87.25409

				213.1		87.23857

				213.12		87.23081

				213.14		87.19589

				213.16		87.19977

				213.18		87.18813

				213.2		87.17649

				213.22		87.16873

				213.24		87.16873

				213.27		87.14932

				213.29		87.1338

				213.31		87.14156

				213.33		87.11828

				213.35		87.10664

				213.37		87.09888

				213.39		87.08336

				213.41		87.0562

				213.43		87.04456

				213.45		87.03292

				213.47		87.02128

				213.5		87.00188

				213.52		86.99024

				213.54		86.98248

				213.56		86.9592

				213.58		86.94756

				213.6		86.9398

				213.62		86.9204

				213.64		86.901

				213.66		86.901

				213.68		86.87772

				213.7		86.8622

				213.73		86.85056

				213.75		86.83892

				213.77		86.8234

				213.79		86.80788

				213.81		86.80012

				213.83		86.77296

				213.85		86.7652

				213.87		86.74968

				213.89		86.73804

				213.91		86.71476

				213.94		86.71088

				213.96		86.69536

				213.98		86.69536

				214		86.65268

				214.02		86.65268

				214.04		86.6294

				214.06		86.61

				214.08		86.58284

				214.1		86.60612

				214.12		86.57896

				214.14		86.56344

				214.17		86.5518

				214.19		86.53628

				214.21		86.50912

				214.23		86.48584

				214.25		86.48196

				214.27		86.45868

				214.29		86.44704

				214.31		86.42376

				214.33		86.42376

				214.35		86.38884

				214.37		86.38884

				214.4		86.38496

				214.42		86.36556

				214.44		86.34616

				214.46		86.3384

				214.48		86.31124

				214.5		86.2802

				214.52		86.28408

				214.54		86.2608

				214.56		86.24916

				214.58		86.2414

				214.6		86.2414

				214.63		86.21812

				214.65		86.21036

				214.67		86.19484

				214.69		86.17932

				214.71		86.15216

				214.73		86.13664

				214.75		86.11724

				214.77		86.11724

				214.79		86.1056

				214.81		86.09396

				214.83		86.07844

				214.86		86.0668

				214.88		86.03963

				214.9		86.02411

				214.92		86.00859

				214.94		85.99695

				214.96		85.98531

				214.98		85.96591

				215		85.95039

				215.02		85.93099

				215.04		85.91159

				215.06		85.89995

				215.09		85.89219

				215.11		85.88443

				215.13		85.86891

				215.15		85.85727

				215.17		85.83787

				215.19		85.81459

				215.21		85.79519

				215.23		85.79907

				215.25		85.76803

				215.27		85.77191

				215.29		85.75639

				215.32		85.75639

				215.34		85.71759

				215.36		85.71371

				215.38		85.67879

				215.4		85.66715

				215.42		85.63999

				215.44		85.63611

				215.46		85.62059

				215.48		85.60119

				215.5		85.57791

				215.52		85.57015

				215.55		85.55075

				215.57		85.53135

				215.59		85.51583

				215.61		85.51971

				215.63		85.49643

				215.65		85.48867

				215.67		85.47703

				215.69		85.47315

				215.71		85.44987

				215.73		85.43047

				215.75		85.40719

				215.78		85.38779

				215.8		85.36451

				215.82		85.35675

				215.84		85.34511

				215.86		85.32959

				215.88		85.31795

				215.9		85.29855

				215.92		85.27915

				215.94		85.26363

				215.96		85.24811

				215.98		85.22871

				216.01		85.21319

				216.03		85.20155

				216.05		85.18603

				216.07		85.17051

				216.09		85.14335

				216.11		85.14335

				216.13		85.11619

				216.15		85.11619

				216.17		85.08127

				216.19		85.08903

				216.21		85.05411

				216.24		85.05023

				216.26		85.01531

				216.28		85.01531

				216.3		84.98815

				216.32		84.98039

				216.34		84.95711

				216.36		84.95711

				216.38		84.93382

				216.4		84.92606

				216.42		84.89502

				216.45		84.88726

				216.47		84.86398

				216.49		84.8407

				216.51		84.81742

				216.53		84.8213

				216.55		84.79802

				216.57		84.77862

				216.59		84.78638

				216.61		84.7631

				216.63		84.7437

				216.65		84.7243

				216.68		84.70878

				216.7		84.6855

				216.72		84.67774

				216.74		84.65446

				216.76		84.65058

				216.78		84.61954

				216.8		84.59626

				216.82		84.5885

				216.84		84.56522

				216.86		84.55358

				216.88		84.54582

				216.91		84.5497

				216.93		84.5109

				216.95		84.51866

				216.97		84.4915

				216.99		84.47598

				217.01		84.44882

				217.03		84.4333

				217.05		84.41002

				217.07		84.38674

				217.09		84.37122

				217.12		84.35182

				217.14		84.34794

				217.16		84.3169

				217.18		84.30526

				217.2		84.28974

				217.22		84.27034

				217.24		84.25094

				217.26		84.24706

				217.28		84.22378

				217.3		84.20438

				217.32		84.18498

				217.35		84.17722

				217.37		84.15394

				217.39		84.14618

				217.41		84.12678

				217.43		84.11126

				217.45		84.09962

				217.47		84.0841

				217.49		84.06858

				217.51		84.05694

				217.53		84.04918

				217.55		84.01814

				217.58		84.01426

				217.6		83.98322

				217.62		83.97158

				217.64		83.94442

				217.66		83.9289

				217.68		83.90174

				217.7		83.8901

				217.72		83.8707

				217.74		83.8513

				217.76		83.83966

				217.79		83.82414

				217.81		83.81249

				217.83		83.80473

				217.85		83.79309

				217.87		83.76981

				217.89		83.75429

				217.91		83.73877

				217.93		83.71937

				217.95		83.69997

				217.97		83.67669

				217.99		83.65729

				218.02		83.65729

				218.04		83.63013

				218.06		83.62237

				218.08		83.60685

				218.1		83.57969

				218.12		83.55253

				218.14		83.54477

				218.16		83.51761

				218.18		83.50597

				218.2		83.50985

				218.23		83.48657

				218.25		83.47105

				218.27		83.44389

				218.29		83.43225

				218.31		83.40121

				218.33		83.38569

				218.35		83.36241

				218.37		83.36629

				218.39		83.33913

				218.41		83.32361

				218.43		83.30421

				218.46		83.28093

				218.48		83.24989

				218.5		83.24213

				218.52		83.21885

				218.54		83.20333

				218.56		83.19169

				218.58		83.19169

				218.6		83.15289

				218.62		83.13349

				218.64		83.11797

				218.66		83.08693

				218.69		83.05977

				218.71		83.05201

				218.73		83.04813

				218.75		83.02097

				218.77		83.01709

				218.79		82.99769

				218.81		82.97829

				218.83		82.94725

				218.85		82.94337

				218.87		82.93173

				218.9		82.90845

				218.92		82.89293

				218.94		82.88517

				218.96		82.86577

				218.98		82.83473

				219		82.84249

				219.02		82.81921

				219.04		82.80757

				219.06		82.78817

				219.08		82.77653

				219.1		82.74937

				219.13		82.72609

				219.15		82.70669

				219.17		82.6834

				219.19		82.65624

				219.21		82.62908

				219.23		82.62132

				219.25		82.59028

				219.27		82.57476

				219.29		82.56312

				219.31		82.54372

				219.34		82.51268

				219.36		82.5088

				219.38		82.49328

				219.4		82.47776

				219.42		82.45836

				219.44		82.46224

				219.46		82.4312

				219.48		82.40404

				219.5		82.40016

				219.52		82.38464

				219.54		82.34584

				219.57		82.34196

				219.59		82.32256

				219.61		82.29152

				219.63		82.26436

				219.65		82.26048

				219.67		82.2372

				219.69		82.2178

				219.71		82.21004

				219.73		82.20228

				219.75		82.18288

				219.78		82.1596

				219.8		82.1596

				219.82		82.13632

				219.84		82.10916

				219.86		82.08976

				219.88		82.082

				219.9		82.0432

				219.92		82.0238

				219.94		82.0238

				219.96		81.97724

				219.99		81.95396

				220.01		81.96172

				220.03		81.94232

				220.05		81.89576

				220.07		81.9074

				220.09		81.89188

				220.11		81.84532

				220.13		81.83756

				220.15		81.83756

				220.17		81.79876

				220.19		81.77936

				220.22		81.77936

				220.24		81.75608

				220.26		81.70952

				220.28		81.71728

				220.3		81.70176

				220.32		81.67072

				220.34		81.63192

				220.36		81.66684

				220.38		81.62416

				220.4		81.60088

				220.43		81.58924

				220.45		81.60088

				220.47		81.53879

				220.49		81.53103

				220.51		81.50775

				220.53		81.47671

				220.55		81.43791

				220.57		81.43791

				220.59		81.41851

				220.61		81.38359

				220.64		81.39135

				220.66		81.37971

				220.68		81.34479

				220.7		81.32539

				220.72		81.33703

				220.74		81.30211

				220.76		81.27495

				220.78		81.26719

				220.8		81.25943

				220.82		81.22839

				220.85		81.20511

				220.87		81.20899

				220.89		81.17795

				220.91		81.14691

				220.93		81.13139

				220.95		81.12751

				220.97		81.07319

				220.99		81.07319

				221.01		81.04603

				221.04		81.03051

				221.06		80.98783

				221.08		80.98783

				221.1		80.96067

				221.12		80.94515

				221.14		80.91799

				221.16		80.92187

				221.18		80.87143

				221.2		80.86367

				221.22		80.85203

				221.24		80.82875

				221.27		80.79771

				221.29		80.80547

				221.31		80.78607

				221.33		80.75891

				221.35		80.73563

				221.37		80.73951

				221.39		80.71235

				221.41		80.67743

				221.43		80.67743

				221.46		80.67355

				221.48		80.62699

				221.5		80.60759

				221.52		80.60371

				221.54		80.56103

				221.56		80.53387

				221.58		80.52999

				221.6		80.49895

				221.62		80.4679

				221.64		80.46014

				221.66		80.44074

				221.69		80.39806

				221.71		80.39418

				221.73		80.37478

				221.75		80.3515

				221.77		80.32434

				221.79		80.3321

				221.81		80.32046

				221.83		80.29718

				221.85		80.28942

				221.88		80.28166

				221.9		80.25062

				221.92		80.21182

				221.94		80.18854

				221.96		80.14974

				221.98		80.12258

				222		80.10706

				222.02		80.0799

				222.04		80.0605

				222.06		80.04886

				222.09		80.03334

				222.11		79.99454

				222.13		79.97902

				222.15		79.97902

				222.17		79.95574

				222.19		79.92858

				222.21		79.93246

				222.23		79.93634

				222.25		79.88978

				222.27		79.87814

				222.3		79.87426

				222.32		79.8277

				222.34		79.79278

				222.36		79.79666

				222.38		79.77726

				222.4		79.72294

				222.42		79.72682

				222.44		79.6919

				222.46		79.6531

				222.48		79.62206

				222.51		79.62982

				222.53		79.59102

				222.55		79.56774

				222.57		79.56774

				222.59		79.55222

				222.61		79.52118

				222.63		79.52118

				222.65		79.52894

				222.67		79.48626

				222.69		79.47074

				222.72		79.46298

				222.74		79.45134

				222.76		79.40866

				222.78		79.40478

				222.8		79.3815

				222.82		79.35045

				222.84		79.32329

				222.86		79.30389

				222.88		79.27285

				222.9		79.24569

				222.93		79.23017

				222.95		79.21077

				222.97		79.17197

				222.99		79.15645

				223.01		79.14093

				223.03		79.10989

				223.05		79.08273

				223.07		79.09437

				223.09		79.07109

				223.11		79.03617

				223.14		79.03229

				223.16		79.01289

				223.18		78.97021

				223.2		78.95081

				223.22		78.95857

				223.24		78.92753

				223.26		78.90425

				223.28		78.89649

				223.3		78.86933

				223.33		78.84217

				223.35		78.82277

				223.37		78.79949

				223.39		78.76457

				223.41		78.75293

				223.43		78.72577

				223.45		78.70249

				223.47		78.67533

				223.49		78.66369

				223.51		78.63265

				223.54		78.58221

				223.56		78.57445

				223.58		78.56281

				223.6		78.52789

				223.62		78.50849

				223.64		78.51237

				223.66		78.48521

				223.68		78.45805

				223.7		78.45805

				223.73		78.43089

				223.75		78.41537

				223.77		78.38433

				223.79		78.36881

				223.81		78.32225

				223.83		78.30285

				223.85		78.27957

				223.87		78.26017

				223.89		78.233

				223.91		78.22136

				223.94		78.20972

				223.96		78.17092

				223.98		78.15152

				224		78.136

				224.02		78.10884

				224.04		78.07004

				224.06		78.07004

				224.08		78.05452

				224.1		78.02348

				224.13		77.99632

				224.15		77.98468

				224.17		77.95752

				224.19		77.91872

				224.21		77.91484

				224.23		77.89544

				224.25		77.87216

				224.27		77.84888

				224.29		77.84112

				224.31		77.80232

				224.34		77.77516

				224.36		77.75188

				224.38		77.72472

				224.4		77.6898

				224.42		77.67816

				224.44		77.66264

				224.46		77.63548

				224.48		77.6122

				224.5		77.60444

				224.53		77.5734

				224.55		77.54236

				224.57		77.52684

				224.59		77.51132

				224.61		77.48028

				224.63		77.46476

				224.65		77.44148

				224.67		77.42596

				224.69		77.3988

				224.71		77.38328

				224.74		77.36

				224.76		77.34448

				224.78		77.31344

				224.8		77.2824

				224.82		77.27464

				224.84		77.23972

				224.86		77.22808

				224.88		77.18928

				224.9		77.17376

				224.93		77.13496

				224.95		77.12331

				224.97		77.08839

				224.99		77.07675

				225.01		77.06899

				225.03		77.04959

				225.05		77.01855

				225.07		76.99915

				225.09		76.99527

				225.11		76.95259

				225.14		76.92931

				225.16		76.90215

				225.18		76.89051

				225.2		76.85171

				225.22		76.85171

				225.24		76.82455

				225.26		76.80515

				225.28		76.77023

				225.3		76.76247

				225.32		76.71979

				225.35		76.70039

				225.37		76.68487

				225.39		76.66159

				225.41		76.60727

				225.43		76.60727

				225.45		76.58399

				225.47		76.54907

				225.49		76.52191

				225.51		76.51803

				225.54		76.48311

				225.56		76.45207

				225.58		76.44819

				225.6		76.43655

				225.62		76.40939

				225.64		76.37835

				225.66		76.37835

				225.68		76.34343

				225.7		76.31239

				225.72		76.30463

				225.75		76.28523

				225.77		76.24643

				225.79		76.21539

				225.81		76.19599

				225.83		76.15331

				225.85		76.13391

				225.87		76.11451

				225.89		76.09899

				225.91		76.07183

				225.93		76.05631

				225.96		76.03303

				225.98		76.01751

				226		75.98258

				226.02		75.97094

				226.04		75.94766

				226.06		75.9205

				226.08		75.89722

				226.1		75.88558

				226.12		75.84678

				226.14		75.83514

				226.17		75.80022

				226.19		75.7847

				226.21		75.75366

				226.23		75.74202

				226.25		75.69546

				226.27		75.68382

				226.29		75.6489

				226.31		75.63338

				226.33		75.60622

				226.35		75.58294

				226.38		75.55966

				226.4		75.52086

				226.42		75.49758

				226.44		75.4743

				226.46		75.45878

				226.48		75.41998

				226.5		75.40834

				226.52		75.38118

				226.54		75.34626

				226.56		75.32686

				226.59		75.2997

				226.61		75.28806

				226.63		75.24926

				226.65		75.2415

				226.67		75.2027

				226.69		75.19494

				226.71		75.1639

				226.73		75.16778

				226.75		75.1251

				226.77		75.09794

				226.8		75.07466

				226.82		75.04362

				226.84		75.00094

				226.86		74.98154

				226.88		74.96214

				226.9		74.93498

				226.92		74.91946

				226.94		74.89618

				226.96		74.87677

				226.98		74.84185

				227.01		74.81857

				227.03		74.79141

				227.05		74.76425

				227.07		74.74485

				227.09		74.72933

				227.11		74.71381

				227.13		74.69053

				227.15		74.65949

				227.17		74.63233

				227.19		74.59741

				227.22		74.56249

				227.24		74.53533

				227.26		74.51981

				227.28		74.48101

				227.3		74.47325

				227.32		74.45385

				227.34		74.42281

				227.36		74.39565

				227.38		74.38013

				227.4		74.36073

				227.43		74.32581

				227.45		74.31029

				227.47		74.28313

				227.49		74.25597

				227.51		74.21717

				227.53		74.20165

				227.55		74.17449

				227.57		74.14733

				227.59		74.12017

				227.61		74.10077

				227.64		74.06585

				227.66		74.04645

				227.68		74.02705

				227.7		73.98825

				227.72		73.96109

				227.74		73.93781

				227.76		73.91453

				227.78		73.87185

				227.8		73.85633

				227.83		73.83305

				227.85		73.81365

				227.87		73.77096

				227.89		73.75932

				227.91		73.7438

				227.93		73.71664

				227.95		73.68172

				227.97		73.67784

				227.99		73.63516

				228.01		73.61188

				228.04		73.57308

				228.06		73.54592

				228.08		73.511

				228.1		73.49936

				228.12		73.46056

				228.14		73.44504

				228.16		73.4334

				228.18		73.414

				228.2		73.3752

				228.22		73.35192

				228.25		73.32476

				228.27		73.29372

				228.29		73.24716

				228.31		73.22776

				228.33		73.20448

				228.35		73.17732

				228.37		73.14628

				228.39		73.13464

				228.41		73.1036

				228.43		73.07256

				228.46		73.04928

				228.48		73.02212

				228.5		72.97556

				228.52		72.97556

				228.54		72.9484

				228.56		72.92124

				228.58		72.88244

				228.6		72.88244

				228.62		72.84364

				228.64		72.82036

				228.67		72.78932

				228.69		72.7738

				228.71		72.74276

				228.73		72.70784

				228.75		72.68068

				228.77		72.65351

				228.79		72.63799

				228.81		72.61083

				228.83		72.57979

				228.85		72.56427

				228.87		72.52935

				228.9		72.49443

				228.92		72.48279

				228.94		72.45951

				228.96		72.42459

				228.98		72.40907

				229		72.38191

				229.02		72.34699

				229.04		72.31983

				229.06		72.30043

				229.08		72.26939

				229.11		72.24223

				229.13		72.21507

				229.15		72.18403

				229.17		72.15687

				229.19		72.13747

				229.21		72.11807

				229.23		72.09091

				229.25		72.05599

				229.27		72.04435

				229.29		72.00167

				229.32		71.97839

				229.34		71.93571

				229.36		71.93183

				229.38		71.88527

				229.4		71.86587

				229.42		71.82707

				229.44		71.81155

				229.46		71.78827

				229.48		71.77275

				229.5		71.73783

				229.53		71.71843

				229.55		71.68351

				229.57		71.64083

				229.59		71.61755

				229.61		71.59815

				229.63		71.56711

				229.65		71.54382

				229.67		71.50502

				229.69		71.47786

				229.71		71.4507

				229.74		71.42354

				229.76		71.40026

				229.78		71.38474

				229.8		71.34594

				229.82		71.32266

				229.84		71.30326

				229.86		71.27222

				229.88		71.24118

				229.9		71.21402

				229.92		71.19074

				229.94		71.15582

				229.97		71.12478

				229.99		71.10926

				230.01		71.07822

				230.03		71.05882

				230.05		71.02002

				230.07		71.00838

				230.09		70.96182

				230.11		70.9463

				230.13		70.91138

				230.15		70.89198

				230.18		70.86094

				230.2		70.84542

				230.22		70.81438

				230.24		70.78722

				230.26		70.77558

				230.28		70.7329

				230.3		70.70186

				230.32		70.66694

				230.34		70.6359

				230.36		70.5971

				230.39		70.56994

				230.41		70.54278

				230.43		70.5195

				230.45		70.5001

				230.47		70.47294

				230.49		70.45742

				230.51		70.41861

				230.53		70.39145

				230.55		70.35653

				230.57		70.33325

				230.6		70.29057

				230.62		70.28281

				230.64		70.24401

				230.66		70.21685

				230.68		70.18581

				230.7		70.17029

				230.72		70.13925

				230.74		70.11597

				230.76		70.07717

				230.78		70.06165

				230.81		70.03061

				230.83		69.99181

				230.85		69.95689

				230.87		69.93361

				230.89		69.89481

				230.91		69.87153

				230.93		69.84049

				230.95		69.82109

				230.97		69.77453

				230.99		69.74737

				231.02		69.72797

				231.04		69.69305

				231.06		69.68141

				231.08		69.66589

				231.1		69.63485

				231.12		69.59993

				231.14		69.59605

				231.16		69.54561

				231.18		69.51845

				231.2		69.49129

				231.23		69.46025

				231.25		69.41369

				231.27		69.37877

				231.29		69.35549

				231.31		69.32833

				231.33		69.30116

				231.35		69.26624

				231.37		69.2546

				231.39		69.20804

				231.41		69.18088

				231.44		69.1382

				231.46		69.12656

				231.48		69.07612

				231.5		69.06448

				231.52		69.0218

				231.54		68.99852

				231.56		68.97136

				231.58		68.95972

				231.6		68.91704

				231.62		68.90152

				231.65		68.87048

				231.67		68.83168

				231.69		68.79288

				231.71		68.76572

				231.73		68.73468

				231.75		68.70752

				231.77		68.68036

				231.79		68.6532

				231.81		68.62992

				231.83		68.58724

				231.86		68.56784

				231.88		68.5368

				231.9		68.50964

				231.92		68.47084

				231.94		68.44756

				231.96		68.401

				231.98		68.3816

				232		68.35444

				232.02		68.3234

				232.04		68.28072

				232.07		68.27296

				232.09		68.23028

				232.11		68.18371

				232.13		68.16819

				232.15		68.15267

				232.17		68.10999

				232.19		68.06731

				232.21		68.05955

				232.23		68.02075

				232.25		67.98195

				232.27		67.94703

				232.3		67.94315

				232.32		67.89659

				232.34		67.86555

				232.36		67.84227

				232.38		67.81511

				232.4		67.77243

				232.42		67.74139

				232.44		67.72199

				232.46		67.67543

				232.48		67.65603

				232.51		67.62887

				232.53		67.60947

				232.55		67.56291

				232.57		67.55515

				232.59		67.51635

				232.61		67.48143

				232.63		67.43099

				232.65		67.42323

				232.67		67.37667

				232.69		67.35727

				232.72		67.32623

				232.74		67.30295

				232.76		67.26027

				232.78		67.23699

				232.8		67.19819

				232.82		67.17491

				232.84		67.14387

				232.86		67.11671

				232.88		67.0779

				232.9		67.04686

				232.92		67.01582

				232.95		66.97314

				232.97		66.94986

				232.99		66.9227

				233.01		66.89554

				233.03		66.84898

				233.05		66.83734

				233.07		66.79466

				233.09		66.77138

				233.11		66.72482

				233.13		66.70154

				233.16		66.66274

				233.18		66.6317

				233.2		66.60066

				233.22		66.5735

				233.24		66.55798

				233.26		66.51918

				233.28		66.49202

				233.3		66.46098

				233.32		66.42994

				233.34		66.38726

				233.37		66.37174

				233.39		66.32906

				233.41		66.29802

				233.43		66.26698

				233.45		66.23982

				233.47		66.1855

				233.49		66.17774

				233.51		66.14282

				233.53		66.1079

				233.55		66.07686

				233.58		66.05746

				233.6		66.01866

				233.62		65.97598

				233.64		65.95269

				233.66		65.92941

				233.68		65.89837

				233.7		65.84405

				233.72		65.83241

				233.74		65.79749

				233.76		65.74705

				233.78		65.71989

				233.81		65.71601

				233.83		65.66557

				233.85		65.63841

				233.87		65.62677

				233.89		65.58409

				233.91		65.54141

				233.93		65.52201

				233.95		65.49097

				233.97		65.44053

				233.99		65.41337

				234.02		65.38621

				234.04		65.34741

				234.06		65.30861

				234.08		65.28533

				234.1		65.25817

				234.12		65.23489

				234.14		65.19221

				234.16		65.17281

				234.18		65.13401

				234.2		65.10685

				234.23		65.06029

				234.25		65.04089

				234.27		64.99821

				234.29		64.96717

				234.31		64.94001

				234.33		64.90897

				234.35		64.87017

				234.37		64.83524

				234.39		64.79644

				234.41		64.75764

				234.44		64.73436

				234.46		64.69168

				234.48		64.65676

				234.5		64.649

				234.52		64.61796

				234.54		64.5714

				234.56		64.54424

				234.58		64.52484

				234.6		64.47828

				234.62		64.42784

				234.65		64.4162

				234.67		64.38904

				234.69		64.34636

				234.71		64.31532

				234.73		64.29592

				234.75		64.25712

				234.77		64.21832

				234.79		64.20668

				234.81		64.164

				234.83		64.14072

				234.85		64.09804

				234.88		64.07476

				234.9		64.03208

				234.92		63.99328

				234.94		63.9506

				234.96		63.92732

				234.98		63.873

				235		63.8342

				235.02		63.81868

				235.04		63.78764

				235.06		63.74108

				235.09		63.7372

				235.11		63.70615

				235.13		63.65959

				235.15		63.62855

				235.17		63.60915

				235.19		63.56259

				235.21		63.51991

				235.23		63.50439

				235.25		63.46559

				235.27		63.42679

				235.3		63.38411

				235.32		63.35695

				235.34		63.31815

				235.36		63.27935

				235.38		63.24443

				235.4		63.22115

				235.42		63.19011

				235.44		63.15131

				235.46		63.12415

				235.48		63.08535

				235.5		63.05431

				235.53		63.01939

				235.55		62.97283

				235.57		62.93015

				235.59		62.90687

				235.61		62.87195

				235.63		62.84091

				235.65		62.81375

				235.67		62.78271

				235.69		62.74003

				235.71		62.70123

				235.74		62.67019

				235.76		62.64691

				235.78		62.6081

				235.8		62.57706

				235.82		62.54602

				235.84		62.50334

				235.86		62.45678

				235.88		62.44126

				235.9		62.40246

				235.92		62.37142

				235.95		62.34038

				235.97		62.32874

				235.99		62.26278

				236.01		62.2395

				236.03		62.20458

				236.05		62.17354

				236.07		62.10758

				236.09		62.09594

				236.11		62.05714

				236.13		62.01058

				236.16		61.97566

				236.18		61.96014

				236.2		61.92134

				236.22		61.87866

				236.24		61.84762

				236.26		61.81658

				236.28		61.7739

				236.3		61.74674

				236.32		61.7157

				236.34		61.69242

				236.36		61.64586

				236.39		61.62646

				236.41		61.5799

				236.43		61.53722

				236.45		61.49453

				236.47		61.47901

				236.49		61.40917

				236.51		61.37813

				236.53		61.35485

				236.55		61.30053

				236.57		61.25397

				236.6		61.23845

				236.62		61.20353

				236.64		61.14921

				236.66		61.12205

				236.68		61.10265

				236.7		61.05997

				236.72		61.02117

				236.74		60.99401

				236.76		60.97073

				236.78		60.91253

				236.81		60.90477

				236.83		60.86209

				236.85		60.83493

				236.87		60.79225

				236.89		60.76121

				236.91		60.70301

				236.93		60.66809

				236.95		60.62929

				236.97		60.59049

				236.99		60.54781

				237.02		60.50901

				237.04		60.48573

				237.06		60.43529

				237.08		60.40037

				237.1		60.37708

				237.12		60.34216

				237.14		60.30336

				237.16		60.26844

				237.18		60.2374

				237.2		60.19472

				237.23		60.17144

				237.25		60.13652

				237.27		60.12488

				237.29		60.07832

				237.31		60.04728

				237.33		60.01236

				237.35		59.9658

				237.37		59.92312

				237.39		59.89984

				237.41		59.87268

				237.43		59.81448

				237.46		59.7912

				237.48		59.7524

				237.5		59.70196

				237.52		59.6554

				237.54		59.636

				237.56		59.58556

				237.58		59.53512

				237.6		59.5196

				237.62		59.48856

				237.64		59.442

				237.67		59.4032

				237.69		59.40708

				237.71		59.34888

				237.73		59.31008

				237.75		59.2868

				237.77		59.26739

				237.79		59.19755

				237.81		59.17815

				237.83		59.16263

				237.85		59.09667

				237.88		59.05399

				237.9		59.03847

				237.92		58.99191

				237.94		58.92595

				237.96		58.91819

				237.98		58.87163

				238		58.82507

				238.02		58.77463

				238.04		58.75135

				238.06		58.70091

				238.09		58.66599

				238.11		58.63883

				238.13		58.60779

				238.15		58.55347

				238.17		58.53407

				238.19		58.50691

				238.21		58.46035

				238.23		58.42931

				238.25		58.41767

				238.27		58.37111

				238.3		58.32455

				238.32		58.30515

				238.34		58.25859

				238.36		58.21203

				238.38		58.17711

				238.4		58.14994

				238.42		58.09562

				238.44		58.06458

				238.46		58.03354

				238.49		57.97922

				238.51		57.93266

				238.53		57.90162

				238.55		57.8667

				238.57		57.80462

				238.59		57.79686

				238.61		57.76194

				238.63		57.71926

				238.65		57.67658

				238.67		57.66494

				238.7		57.61062

				238.72		57.56794

				238.74		57.52526

				238.76		57.49034

				238.78		57.4399

				238.8		57.39722

				238.82		57.35842

				238.84		57.33902

				238.86		57.27306

				238.88		57.24978

				238.91		57.21486

				238.93		57.17606

				238.95		57.12562

				238.97		57.12562

				238.99		57.06742

				239.01		57.02861

				239.03		57.00921

				239.05		56.96653

				239.07		56.91221

				239.1		56.88505

				239.12		56.87341

				239.14		56.81521

				239.16		56.76865

				239.18		56.72985

				239.2		56.71045

				239.22		56.64449

				239.24		56.61345

				239.26		56.58241

				239.29		56.54361

				239.31		56.48541

				239.33		56.45825

				239.35		56.40781

				239.37		56.36901

				239.39		56.34185

				239.41		56.29917

				239.43		56.24485

				239.45		56.20217

				239.47		56.16725

				239.5		56.11681

				239.52		56.10905

				239.54		56.11293

				239.56		56.07801

				239.58		56.00041

				239.6		55.96161

				239.62		55.9034

				239.64		55.81416

				239.66		55.787

				239.69		55.79088

				239.71		55.7676

				239.73		55.71716

				239.75		55.69388

				239.77		55.64732

				239.79		55.62016

				239.81		55.56972

				239.83		55.53092

				239.85		55.48436

				239.87		55.43392

				239.9		55.39124

				239.92		55.35632

				239.94		55.30588

				239.96		55.2826

				239.98		55.25544

				240		55.19724

				240.02		55.14292

				240.04		55.1468

				240.06		55.0886

				240.09		55.04204

				240.11		55.02652

				240.13		55.00324

				240.15		54.9334

				240.17		54.88296

				240.19		54.87132

				240.21		54.817

				240.23		54.77431

				240.25		54.74327

				240.28		54.73163

				240.3		54.66179

				240.32		54.63075

				240.34		54.59195

				240.36		54.54539

				240.38		54.48719

				240.4		54.47167

				240.42		54.42123

				240.44		54.37855

				240.47		54.33587

				240.49		54.31259

				240.51		54.25051

				240.53		54.21171

				240.55		54.17291

				240.57		54.14187

				240.59		54.08755

				240.61		54.05651

				240.63		54.03323

				240.65		53.98667

				240.68		53.95175

				240.7		53.92071

				240.72		53.88967

				240.74		53.82759

				240.76		53.80431

				240.78		53.75775

				240.8		53.70731

				240.82		53.6685

				240.84		53.6297

				240.87		53.57538

				240.89		53.52882

				240.91		53.4939

				240.93		53.4357

				240.95		53.38914

				240.97		53.34646

				240.99		53.30766

				241.01		53.2611

				241.03		53.24558

				241.06		53.20678

				241.08		53.1641

				241.1		53.11754

				241.12		53.09038

				241.14		53.03606

				241.16		52.99726

				241.18		52.95458

				241.2		52.92354

				241.22		52.86922

				241.25		52.82266

				241.27		52.7955

				241.29		52.75282

				241.31		52.70238

				241.33		52.66746

				241.35		52.62866

				241.37		52.56269

				241.39		52.53165

				241.41		52.49673

				241.43		52.44629

				241.46		52.39973

				241.48		52.38033

				241.5		52.33377

				241.52		52.28721

				241.54		52.24453

				241.56		52.21737

				241.58		52.17081

				241.6		52.12037

				241.62		52.08933

				241.65		52.06217

				241.67		52.01173

				241.69		51.96905

				241.71		51.94577

				241.73		51.88757

				241.75		51.83325

				241.77		51.79057

				241.79		51.75177

				241.81		51.69357

				241.84		51.67029

				241.86		51.61597

				241.88		51.58881

				241.9		51.52673

				241.92		51.49957

				241.94		51.44136

				241.96		51.4142

				241.98		51.37152

				242		51.34048

				242.03		51.29004

				242.05		51.24736

				242.07		51.21244

				242.09		51.162

				242.11		51.14648

				242.13		51.09216

				242.15		51.07276

				242.17		51.01844

				242.19		50.97576

				242.22		50.91756

				242.24		50.89816

				242.26		50.84772

				242.28		50.81668

				242.3		50.7546

				242.32		50.7158

				242.34		50.66536

				242.36		50.61104

				242.38		50.56448

				242.41		50.53344

				242.43		50.48688

				242.45		50.44032

				242.47		50.39764

				242.49		50.3666

				242.51		50.32391

				242.53		50.26571

				242.55		50.22691

				242.57		50.19975

				242.59		50.14543

				242.62		50.09499

				242.64		50.07947

				242.66		50.03291

				242.68		49.97859

				242.7		49.92815

				242.72		49.89711

				242.74		49.82339

				242.76		49.79235

				242.78		49.75355

				242.81		49.70699

				242.83		49.66819

				242.85		49.64103

				242.87		49.60223

				242.89		49.54403

				242.91		49.52075

				242.93		49.47031

				242.95		49.42763

				242.97		49.37719

				243		49.35003

				243.02		49.29959

				243.04		49.25691

				243.06		49.1987

				243.08		49.16378

				243.1		49.1017

				243.12		49.07454

				243.14		49.02798

				243.16		48.99694

				243.19		48.94262

				243.21		48.90382

				243.23		48.84174

				243.25		48.80682

				243.27		48.76802

				243.29		48.7137

				243.31		48.6749

				243.33		48.6361

				243.35		48.58954

				243.38		48.52746

				243.4		48.51194

				243.42		48.45762

				243.44		48.42658

				243.46		48.35674

				243.48		48.33346

				243.5		48.2675

				243.52		48.2287

				243.54		48.1705

				243.57		48.1511

				243.59		48.09289

				243.61		48.05409

				243.63		48.00753

				243.65		47.96097

				243.67		47.90665

				243.69		47.87173

				243.71		47.82129

				243.73		47.79025

				243.76		47.75145

				243.78		47.70877

				243.8		47.66609

				243.82		47.61953

				243.84		47.57685

				243.86		47.53029

				243.88		47.47985

				243.9		47.43329

				243.92		47.39449

				243.95		47.34405

				243.97		47.29361

				243.99		47.25481

				244.01		47.20437

				244.03		47.15393

				244.05		47.10349

				244.07		47.06857

				244.09		47.02201

				244.11		46.9832

				244.14		46.93276

				244.16		46.90172

				244.18		46.85128

				244.2		46.81248

				244.22		46.75816

				244.24		46.731

				244.26		46.6728

				244.28		46.62624

				244.3		46.57968

				244.33		46.54476

				244.35		46.4982

				244.37		46.4594

				244.39		46.42448

				244.41		46.3624

				244.43		46.31584

				244.45		46.25764

				244.47		46.2266

				244.49		46.16064

				244.52		46.1296

				244.54		46.08304

				244.56		46.0326

				244.58		45.9744

				244.6		45.94336

				244.62		45.90068

				244.64		45.86575

				244.66		45.83083

				244.68		45.78427

				244.71		45.73383

				244.73		45.66787

				244.75		45.62907

				244.77		45.57863

				244.79		45.53983

				244.81		45.48939

				244.83		45.45835

				244.85		45.40403

				244.87		45.35747

				244.9		45.29539

				244.92		45.26047

				244.94		45.21779

				244.96		45.16347

				244.98		45.11303

				245		45.07811

				245.02		45.01603

				245.04		44.97723

				245.06		44.92291

				245.09		44.89187

				245.11		44.83367

				245.13		44.79875

				245.15		44.7483

				245.17		44.70562

				245.19		44.64742

				245.21		44.6125

				245.23		44.56982

				245.25		44.51162

				245.28		44.4767

				245.3		44.42626

				245.32		44.38358

				245.34		44.33314

				245.36		44.29822

				245.38		44.2439

				245.4		44.19346

				245.42		44.15078

				245.44		44.10034

				245.47		44.05378

				245.49		44.00334

				245.51		43.96842

				245.53		43.90634

				245.55		43.86366

				245.57		43.80158

				245.59		43.77442

				245.61		43.71622

				245.63		43.68906

				245.66		43.62697

				245.68		43.59205

				245.7		43.52997

				245.72		43.49117

				245.74		43.42133

				245.76		43.40581

				245.78		43.34761

				245.8		43.30105

				245.82		43.23509

				245.85		43.21181

				245.87		43.13809

				245.89		43.09541

				245.91		43.04885

				245.93		43.02169

				245.95		42.96737

				245.97		42.92469

				245.99		42.88201

				246.01		42.82769

				246.04		42.78113

				246.06		42.73069

				246.08		42.68801

				246.1		42.64533

				246.12		42.60265

				246.14		42.54445

				246.16		42.50564

				246.18		42.44356

				246.2		42.40088

				246.23		42.35432

				246.25		42.30776

				246.27		42.26896

				246.29		42.23404

				246.31		42.17196

				246.33		42.11376

				246.35		42.0866

				246.37		42.02452

				246.39		41.97408

				246.41		41.9314

				246.44		41.90424

				246.46		41.84604

				246.48		41.7956

				246.5		41.7374

				246.52		41.6986

				246.54		41.63264

				246.56		41.58996

				246.58		41.53952

				246.6		41.50072

				246.63		41.43864

				246.65		41.40371

				246.67		41.34939

				246.69		41.29895

				246.71		41.26015

				246.73		41.19807

				246.75		41.15539

				246.77		41.10107

				246.79		41.06615

				246.82		41.01183

				246.84		40.98079

				246.86		40.93423

				246.88		40.88379

				246.9		40.82171

				246.92		40.76351

				246.94		40.72859

				246.96		40.65487

				246.98		40.61219

				247.01		40.56175

				247.03		40.52295

				247.05		40.46087

				247.07		40.42983

				247.09		40.37163

				247.11		40.33671

				247.13		40.2785

				247.15		40.23582

				247.17		40.17374

				247.2		40.13882

				247.22		40.09614

				247.24		40.04958

				247.26		39.99526

				247.28		39.95646

				247.3		39.92542

				247.32		39.85558

				247.34		39.8129

				247.36		39.78186

				247.38		39.72366

				247.41		39.66158

				247.43		39.61502

				247.45		39.5607

				247.47		39.49474

				247.49		39.45982

				247.51		39.40162

				247.53		39.3667

				247.55		39.30074

				247.57		39.26194

				247.6		39.19986

				247.62		39.15329

				247.64		39.09121

				247.66		39.06017

				247.68		38.99033

				247.7		38.94765

				247.72		38.90109

				247.74		38.83125

				247.76		38.78081

				247.79		38.76529

				247.81		38.71097

				247.83		38.65665

				247.85		38.63337

				247.87		38.58681

				247.89		38.52473

				247.91		38.47429

				247.93		38.43937

				247.95		38.37341

				247.98		38.30745

				248		38.26477

				248.02		38.21045

				248.04		38.14449

				248.06		38.11345

				248.08		38.07853

				248.1		38.00092

				248.12		37.95436

				248.14		37.91556

				248.16		37.86124

				248.19		37.78752

				248.21		37.76812

				248.23		37.72544

				248.25		37.675

				248.27		37.62456

				248.29		37.60128

				248.31		37.5392

				248.33		37.47712

				248.35		37.43832

				248.38		37.37624

				248.4		37.31028

				248.42		37.25596

				248.44		37.2094

				248.46		37.13568

				248.48		37.08524

				248.5		37.05032

				248.52		36.99212

				248.54		36.93391

				248.57		36.89899

				248.59		36.85631

				248.61		36.79035

				248.63		36.74767

				248.65		36.70499

				248.67		36.65455

				248.69		36.58471

				248.71		36.53427

				248.73		36.48383

				248.75		36.41787

				248.78		36.36355

				248.8		36.33251

				248.82		36.28207

				248.84		36.23163

				248.86		36.19283

				248.88		36.15403

				248.9		36.08419

				248.92		36.05315

				248.94		35.99495

				248.97		35.94451

				248.99		35.88243

				249.01		35.84751

				249.03		35.77378

				249.05		35.72722

				249.07		35.68066

				249.09		35.6341

				249.11		35.57202

				249.13		35.52158

				249.15		35.48278

				249.18		35.41294

				249.2		35.35862

				249.22		35.30818

				249.24		35.25774

				249.26		35.18402

				249.28		35.16074

				249.3		35.1103

				249.32		35.06374

				249.34		34.9939

				249.37		34.98226

				249.39		34.90078

				249.41		34.8387

				249.43		34.7999

				249.45		34.76886

				249.47		34.68737

				249.49		34.64469

				249.51		34.61365

				249.53		34.55545

				249.56		34.47397

				249.58		34.42741

				249.6		34.38861

				249.62		34.31101

				249.64		34.25669

				249.66		34.23341

				249.68		34.17909

				249.7		34.10149

				249.72		34.07045

				249.74		34.02001

				249.77		33.95793

				249.79		33.89973

				249.81		33.87645

				249.83		33.79885

				249.85		33.74065

				249.87		33.69409

				249.89		33.64753

				249.91		33.5738

				249.93		33.52336

				249.96		33.48844

				249.98		33.4186

				250		33.36816

				250.02		33.31772

				250.04		33.27504

				250.06		33.21296

				250.08		33.18192

				250.1		33.1082

				250.12		33.05776

				250.15		32.99568

				250.17		32.94912

				250.19		32.87928

				250.21		32.84824

				250.23		32.78228

				250.25		32.73184

				250.27		32.67752

				250.29		32.63096

				250.31		32.57664

				250.33		32.53008

				250.36		32.48351

				250.38		32.44859

				250.4		32.37875

				250.42		32.31667

				250.44		32.27787

				250.46		32.22743

				250.48		32.14207

				250.5		32.11103

				250.52		32.06059

				250.55		31.99463

				250.57		31.94031

				250.59		31.91315

				250.61		31.83555

				250.63		31.77735

				250.65		31.73467

				250.67		31.68035

				250.69		31.60275

				250.71		31.56783

				250.73		31.53679

				250.76		31.47471

				250.78		31.41263

				250.8		31.38547

				250.82		31.34666

				250.84		31.26906

				250.86		31.21086

				250.88		31.17982

				250.9		31.0867

				250.92		31.02462

				250.95		30.98582

				250.97		30.94314

				250.99		30.8539

				251.01		30.8345

				251.03		30.7763

				251.05		30.70646

				251.07		30.6405

				251.09		30.60946

				251.11		30.5435

				251.13		30.48918

				251.16		30.43486

				251.18		30.3883

				251.2		30.31846

				251.22		30.2719

				251.24		30.22921

				251.26		30.17101

				251.28		30.11669

				251.3		30.08177

				251.32		30.02357

				251.35		29.96149

				251.37		29.90717

				251.39		29.85285

				251.41		29.79853

				251.43		29.74033

				251.45		29.68601

				251.47		29.63945

				251.49		29.58513

				251.51		29.53857

				251.53		29.46873

				251.56		29.41829

				251.58		29.35621

				251.6		29.30965

				251.62		29.22041

				251.64		29.19325

				251.66		29.13116

				251.68		29.08848

				251.7		29.0264

				251.72		28.99924

				251.74		28.93716

				251.77		28.87896

				251.79		28.82076

				251.81		28.7742

				251.83		28.71988

				251.85		28.6578

				251.87		28.60736

				251.89		28.5608

				251.91		28.49484

				251.93		28.4444

				251.95		28.39396

				251.98		28.33964

				252		28.2698

				252.02		28.22324

				252.04		28.16892

				252.06		28.10296

				252.08		28.05252

				252.1		28.00595

				252.12		27.93611

				252.14		27.87791

				252.17		27.83523

				252.19		27.78091

				252.21		27.70331

				252.23		27.66063

				252.25		27.61407

				252.27		27.54423

				252.29		27.48215

				252.31		27.46663

				252.33		27.41231

				252.35		27.35411

				252.38		27.29203

				252.4		27.25323

				252.42		27.16787

				252.44		27.11355

				252.46		27.05535

				252.48		27.00879

				252.5		26.93895

				252.52		26.90014

				252.54		26.83418

				252.56		26.7721

				252.59		26.72166

				252.61		26.67122

				252.63		26.60526

				252.65		26.54318

				252.67		26.50438

				252.69		26.45006

				252.71		26.3647

				252.73		26.32978

				252.75		26.28322

				252.78		26.21338

				252.8		26.13966

				252.82		26.11638

				252.84		26.04266

				252.86		25.98834

				252.88		25.92238

				252.9		25.89134

				252.92		25.82538

				252.94		25.76717

				252.96		25.71673

				252.99		25.65465

				253.01		25.59645

				253.03		25.54601

				253.05		25.48393

				253.07		25.41797

				253.09		25.37529

				253.11		25.31321

				253.13		25.23949

				253.15		25.19293

				253.17		25.15025

				253.2		25.09593

				253.22		25.02221

				253.24		24.98341

				253.26		24.92133

				253.28		24.85149

				253.3		24.78941

				253.32		24.75449

				253.34		24.69241

				253.36		24.6342

				253.38		24.576

				253.41		24.52556

				253.43		24.44796

				253.45		24.39364

				253.47		24.33544

				253.49		24.27724

				253.51		24.21128

				253.53		24.1686

				253.55		24.09488

				253.57		24.0328

				253.59		23.97848

				253.62		23.92416

				253.64		23.85044

				253.66		23.79224

				253.68		23.7418

				253.7		23.6836

				253.72		23.606

				253.74		23.55167

				253.76		23.51675

				253.78		23.44691

				253.8		23.38095

				253.83		23.34215

				253.85		23.29947

				253.87		23.22187

				253.89		23.15979

				253.91		23.09771

				253.93		23.03563

				253.95		22.95803

				253.97		22.89207

				253.99		22.83775

				254.02		22.77179

				254.04		22.71359

				254.06		22.64763

				254.08		22.58943

				254.1		22.53123

				254.12		22.48467

				254.14		22.40318

				254.16		22.3605

				254.18		22.3023

				254.2		22.2441

				254.23		22.17426

				254.25		22.13934

				254.27		22.08114

				254.29		22.0113

				254.31		21.95698

				254.33		21.89878

				254.35		21.84058

				254.37		21.76298

				254.39		21.71254

				254.41		21.65046

				254.44		21.58838

				254.46		21.5069

				254.48		21.46034

				254.5		21.37498

				254.52		21.32065

				254.54		21.26633

				254.56		21.20425

				254.58		21.13053

				254.6		21.09173

				254.63		21.02189

				254.65		20.94817

				254.67		20.89385

				254.69		20.84729

				254.71		20.78133

				254.73		20.71149

				254.75		20.66105

				254.77		20.60673

				254.79		20.53689

				254.81		20.46705

				254.84		20.42049

				254.86		20.35065

				254.88		20.27305

				254.9		20.21484

				254.92		20.1644

				254.94		20.09068

				254.96		20.03636

				254.98		19.97428

				255		19.90056

				255.02		19.84236

				255.05		19.78416

				255.07		19.71432

				255.09		19.65612

				255.11		19.6018

				255.13		19.53584

				255.15		19.46212

				255.17		19.4078

				255.19		19.3496

				255.21		19.27976

				255.23		19.22544

				255.26		19.15172

				255.28		19.10516

				255.3		19.03143

				255.32		18.97711

				255.34		18.90339

				255.36		18.86071

				255.38		18.78311

				255.4		18.73655

				255.42		18.65119

				255.44		18.60463

				255.47		18.53867

				255.49		18.47659

				255.51		18.39899

				255.53		18.35631

				255.55		18.28259

				255.57		18.19723

				255.59		18.13515

				255.61		18.08471

				255.63		18.01875

				255.65		17.93338

				255.68		17.90622

				255.7		17.82862

				255.72		17.75102

				255.74		17.66954

				255.76		17.62686

				255.78		17.54926

				255.8		17.49106

				255.82		17.4251

				255.84		17.37078

				255.87		17.30094

				255.89		17.23498

				255.91		17.18454

				255.93		17.1147

				255.95		17.05262

				255.97		16.99054

				255.99		16.92846

				256.01		16.85085

				256.03		16.80429

				256.05		16.73833

				256.08		16.66073

				256.1		16.59477

				256.12		16.54433

				256.14		16.47061

				256.16		16.40853

				256.18		16.33869

				256.2		16.28825

				256.22		16.21453

				256.24		16.15245

				256.26		16.07485

				256.29		16.03217

				256.31		15.94293

				256.33		15.88085

				256.35		15.81877

				256.37		15.7528

				256.39		15.67908

				256.41		15.617

				256.43		15.55492

				256.45		15.47732

				256.47		15.41524

				256.5		15.3454

				256.52		15.28332

				256.54		15.21348

				256.56		15.15528

				256.58		15.0932

				256.6		15.02724

				256.62		14.96904

				256.64		14.91084

				256.66		14.83712

				256.68		14.7634

				256.71		14.71296

				256.73		14.63147

				256.75		14.57327

				256.77		14.50731

				256.79		14.45299

				256.81		14.37539

				256.83		14.32495

				256.85		14.25123

				256.87		14.17751

				256.89		14.10767

				256.92		14.04559

				256.94		13.96799

				256.96		13.90203

				256.98		13.83607

				257		13.77787

				257.02		13.69639

				257.04		13.64983

				257.06		13.59163

				257.08		13.52567

				257.1		13.44806

				257.13		13.4015

				257.15		13.3239

				257.17		13.2463

				257.19		13.19198

				257.21		13.12214

				257.23		13.06006

				257.25		12.99022

				257.27		12.94366

				257.29		12.86994

				257.31		12.81562

				257.34		12.73414

				257.36		12.67206

				257.38		12.59446

				257.4		12.52074

				257.42		12.45866

				257.44		12.39269

				257.46		12.31897

				257.48		12.24913

				257.5		12.17929

				257.53		12.10169

				257.55		12.02797

				257.57		11.96589

				257.59		11.89993

				257.61		11.82621

				257.63		11.76801

				257.65		11.70593

				257.67		11.65161

				257.69		11.57401

				257.71		11.52745

				257.74		11.44597

				257.76		11.38777

				257.78		11.30241

				257.8		11.24808

				257.82		11.1666

				257.84		11.1084

				257.86		11.02692

				257.88		10.97648

				257.9		10.89888

				257.92		10.8368

				257.95		10.76308

				257.97		10.701

				257.99		10.6234

				258.01		10.54968

				258.03		10.49148

				258.05		10.41776

				258.07		10.3518

				258.09		10.28584

				258.11		10.21988

				258.14		10.15391

				258.16		10.08407

				258.18		10.01035

				258.2		9.940513

				258.22		9.882312

				258.24		9.804712

				258.26		9.750391

				258.28		9.680551

				258.3		9.61459

				258.32		9.540869

				258.35		9.478789

				258.37		9.401188

				258.39		9.335227

				258.41		9.269267

				258.43		9.211066

				258.45		9.133466

				258.47		9.067505

				258.49		9.001544

				258.51		8.935584

				258.53		8.873503

				258.56		8.799783

				258.58		8.726062

				258.6		8.671742

				258.62		8.582501

				258.64		8.5243

				258.66		8.45834

				258.68		8.388499

				258.7		8.310898

				258.72		8.264338

				258.74		8.186737

				258.77		8.113017

				258.79		8.054816

				258.81		7.992735

				258.83		7.919015

				258.85		7.829774

				258.87		7.783214

				258.89		7.701733

				258.91		7.624132

				258.93		7.565932

				258.96		7.499971

				258.98		7.42625

				259		7.36805

				259.02		7.294329

				259.04		7.224489

				259.06		7.166288

				259.08		7.088687

				259.1		7.038247

				259.12		6.972286

				259.14		6.894686

				259.17		6.836485

				259.19		6.774405

				259.21		6.692924

				259.23		6.623083

				259.25		6.572643

				259.27		6.498922

				259.29		6.432961

				259.31		6.359241

				259.33		6.29716

				259.35		6.21956

				259.38		6.149719

				259.4		6.087638

				259.42		6.029438

				259.44		5.963477

				259.46		5.889757

				259.48		5.850956

				259.5		5.769475

				259.52		5.687995

				259.54		5.633674

				259.56		5.575474

				259.59		5.486233

				259.61		5.420272

				259.63		5.377592

				259.65		5.303871

				259.67		5.245671

				259.69		5.17195

				259.71		5.12539

				259.73		5.047789

				259.75		4.985708

				259.77		4.908108

				259.8		4.857667

				259.82		4.783947

				259.84		4.729626

				259.86		4.663666

				259.88		4.609345

				259.9		4.539504

				259.92		4.473544

				259.94		4.411463

				259.96		4.353263

				259.98		4.287302

				260		4.221342

				260.03		4.178661

				260.05		4.112701

				260.07		4.0545

				260.09		4.00406

				260.11		3.945859

				260.13		3.883779

				260.15		3.813938

				260.17		3.751857

				260.19		3.693657

				260.21		3.631576

				260.24		3.565616

				260.26		3.519055

				260.28		3.449215

				260.3		3.383254

				260.32		3.344454

				260.34		3.294013

				260.36		3.208653

				260.38		3.185372

				260.4		3.115532

				260.42		3.053451

				260.45		2.999131

				260.47		2.97585

				260.49		2.90989

				260.51		2.88273

				260.53		2.840049

				260.55		2.797369

				260.57		2.723648

				260.59		2.673208

				260.61		2.638287

				260.63		2.572327

				260.65		2.514126

				260.68		2.490846

				260.7		2.455926

				260.72		2.393845

				260.74		2.358925

				260.76		2.327885

				260.78		2.285204

				260.8		2.234764

				260.82		2.211484

				260.84		2.180443

				260.86		2.145523

				260.89		2.114483

				260.91		2.102843

				260.93		2.075682

				260.95		2.029122

				260.97		2.025242

				260.99		2.001962

				261.01		1.963161

				261.03		1.936001

				261.05		1.936001

				261.07		1.893321

				261.09		1.873921

				261.12		1.85452

				261.14		1.839

				261.16		1.8196

				261.18		1.81184

				261.2		1.78468

				261.22		1.7808

				261.24		1.749759

				261.26		1.734239

				261.28		1.707079

				261.3		1.707079

				261.32		1.676039

				261.35		1.679919

				261.37		1.668279

				261.39		1.668279

				261.41		1.652759

				261.43		1.652759

				261.45		1.641118

				261.47		1.625598

				261.49		1.613958

				261.51		1.602318

				261.53		1.606198

				261.55		1.598438

				261.58		1.579038

				261.6		1.571278

				261.62		1.575158

				261.64		1.559638

				261.66		1.536358

				261.68		1.547998

				261.7		1.524717

				261.72		1.532478

				261.74		1.528597

				261.76		1.509197

				261.78		1.520837

				261.8		1.516957

				261.83		1.528597

				261.85		1.516957

				261.87		1.520837

				261.89		1.509197

				261.91		1.505317

				261.93		1.516957

				261.95		1.513077

				261.97		1.513077

				261.99		1.509197

				262.01		1.497557

				262.03		1.501437

				262.06		1.501437

				262.08		1.493677

				262.1		1.493677

				262.12		1.493677

				262.14		1.489797

				262.16		1.485917

				262.18		1.482037

				262.2		1.485917

				262.22		1.482037

				262.24		1.482037

				262.26		1.482037

				262.28		1.478157

				262.31		1.474277

				262.33		1.470397

				262.35		1.474277

				262.37		1.470397

				262.39		1.466517

				262.41		1.466517

				262.43		1.462637

				262.45		1.462637

				262.47		1.462637

				262.49		1.458757

				262.51		1.458757

				262.53		1.458757

				262.56		1.458757

				262.58		1.454877

				262.6		1.454877

				262.62		1.454877

				262.64		1.450997

				262.66		1.450997

				262.68		1.447117

				262.7		1.447117

				262.72		1.447117

				262.74		1.443237

				262.76		1.439357

				262.79		1.443237

				262.81		1.439357

				262.83		1.439357

				262.85		1.435477

				262.87		1.435477

				262.89		1.435477

				262.91		1.435477

				262.93		1.435477

				262.95		1.435477

				262.97		1.435477

				262.99		1.435477

				263.01		1.435477

				263.04		1.435477

				263.06		1.431597

				263.08		1.431597

				263.1		1.431597

				263.12		1.431597

				263.14		1.427717

				263.16		1.427717

				263.18		1.427717

				263.2		1.427717

				263.22		1.423837

				263.24		1.423837

				263.26		1.423837

				263.28		1.423837

				263.31		1.423837

				263.33		1.419957

				263.35		1.419957

				263.37		1.419957

				263.39		1.419957

				263.41		1.419957

				263.43		1.419957

				263.45		1.416076

				263.47		1.416076

				263.49		1.416076

				263.51		1.416076

				263.53		1.416076

				263.56		1.412196

				263.58		1.412196

				263.6		1.412196

				263.62		1.412196

				263.64		1.412196

				263.66		1.412196

				263.68		1.412196

				263.7		1.408316

				263.72		1.408316

				263.74		1.404436

				263.76		1.408316

				263.78		1.404436

				263.81		1.404436

				263.83		1.404436

				263.85		1.404436

				263.87		1.400556

				263.89		1.404436

				263.91		1.400556

				263.93		1.400556

				263.95		1.400556

				263.97		1.400556

				263.99		1.396676

				264.01		1.396676

				264.03		1.396676

				264.06		1.392796

				264.08		1.392796

				264.1		1.392796

				264.12		1.388916

				264.14		1.388916

				264.16		1.388916

				264.18		1.385036

				264.2		1.385036

				264.22		1.385036

				264.24		1.385036

				264.26		1.385036

				264.28		1.385036

				264.31		1.385036

				264.33		1.385036

				264.35		1.385036

				264.37		1.385036

				264.39		1.385036

				264.41		1.385036

				264.43		1.385036

				264.45		1.385036

				264.47		1.385036

				264.49		1.381156

				264.51		1.381156

				264.53		1.381156

				264.55		1.377276

				264.58		1.377276

				264.6		1.377276

				264.62		1.373396

				264.64		1.373396

				264.66		1.373396

				264.68		1.373396

				264.7		1.373396

				264.72		1.373396

				264.74		1.373396

				264.76		1.373396

				264.78		1.369516

				264.8		1.369516

				264.83		1.369516

				264.85		1.369516

				264.87		1.365636

				264.89		1.369516

				264.91		1.365636

				264.93		1.365636

				264.95		1.365636

				264.97		1.365636

				264.99		1.365636

				265.01		1.361756

				265.03		1.365636

				265.05		1.361756

				265.08		1.361756

				265.1		1.361756

				265.12		1.361756

				265.14		1.361756

				265.16		1.357876

				265.18		1.361756

				265.2		1.357876

				265.22		1.357876

				265.24		1.357876

				265.26		1.357876

				265.28		1.357876

				265.3		1.357876

				265.33		1.353996

				265.35		1.353996

				265.37		1.353996

				265.39		1.353996

				265.41		1.350116

				265.43		1.350116

				265.45		1.350116

				265.47		1.350116

				265.49		1.350116

				265.51		1.350116

				265.53		1.350116

				265.55		1.350116

				265.58		1.350116

				265.6		1.350116

				265.62		1.350116

				265.64		1.350116

				265.66		1.350116

				265.68		1.346236

				265.7		1.346236

				265.72		1.346236

				265.74		1.346236

				265.76		1.346236

				265.78		1.346236

				265.8		1.342356

				265.83		1.342356

				265.85		1.342356

				265.87		1.342356

				265.89		1.342356

				265.91		1.338476

				265.93		1.338476

				265.95		1.338476

				265.97		1.338476

				265.99		1.338476

				266.01		1.338476

				266.03		1.338476

				266.05		1.338476

				266.08		1.334596

				266.1		1.334596

				266.12		1.334596

				266.14		1.334596

				266.16		1.334596

				266.18		1.334596

				266.2		1.334596

				266.22		1.334596

				266.24		1.334596

				266.26		1.334596

				266.28		1.334596

				266.3		1.334596

				266.32		1.334596

				266.35		1.334596

				266.37		1.334596

				266.39		1.334596

				266.41		1.330716

				266.43		1.330716

				266.45		1.330716

				266.47		1.330716

				266.49		1.330716

				266.51		1.330716

				266.53		1.330716

				266.55		1.326836

				266.57		1.326836

				266.6		1.326836

				266.62		1.326836

				266.64		1.326836

				266.66		1.322956

				266.68		1.322956

				266.7		1.322956

				266.72		1.322956

				266.74		1.322956

				266.76		1.322956

				266.78		1.322956

				266.8		1.322956

				266.82		1.319076

				266.85		1.319076

				266.87		1.319076

				266.89		1.319076

				266.91		1.319076

				266.93		1.319076

				266.95		1.319076

				266.97		1.319076

				266.99		1.315196

				267.01		1.315196

				267.03		1.315196

				267.05		1.315196

				267.07		1.315196

				267.09		1.315196

				267.12		1.315196

				267.14		1.315196

				267.16		1.315196

				267.18		1.315196

				267.2		1.315196

				267.22		1.315196

				267.24		1.311316

				267.26		1.311316

				267.28		1.311316

				267.3		1.311316

				267.32		1.311316

				267.34		1.307436

				267.37		1.307436

				267.39		1.307436

				267.41		1.307436

				267.43		1.307436

				267.45		1.307436

				267.47		1.303555

				267.49		1.303555

				267.51		1.303555

				267.53		1.303555

				267.55		1.303555

				267.57		1.299675

				267.59		1.299675

				267.62		1.299675

				267.64		1.299675

				267.66		1.299675

				267.68		1.299675

				267.7		1.295795

				267.72		1.295795

				267.74		1.295795

				267.76		1.295795

				267.78		1.295795

				267.8		1.295795

				267.82		1.295795

				267.84		1.295795

				267.87		1.295795

				267.89		1.295795

				267.91		1.295795

				267.93		1.295795

				267.95		1.291915

				267.97		1.291915

				267.99		1.291915

				268.01		1.291915

				268.03		1.291915

				268.05		1.291915

				268.07		1.291915

				268.09		1.291915

				268.11		1.291915

				268.14		1.291915

				268.16		1.291915

				268.18		1.291915

				268.2		1.291915

				268.22		1.291915

				268.24		1.288035

				268.26		1.288035

				268.28		1.288035

				268.3		1.288035

				268.32		1.288035

				268.34		1.288035

				268.36		1.288035

				268.39		1.288035

				268.41		1.288035

				268.43		1.288035

				268.45		1.284155

				268.47		1.284155

				268.49		1.284155

				268.51		1.284155

				268.53		1.284155

				268.55		1.284155

				268.57		1.284155

				268.59		1.284155

				268.61		1.284155

				268.64		1.280275

				268.66		1.284155

				268.68		1.280275

				268.7		1.280275

				268.72		1.280275

				268.74		1.280275

				268.76		1.280275

				268.78		1.280275

				268.8		1.280275

				268.82		1.280275

				268.84		1.280275

				268.86		1.280275

				268.88		1.280275

				268.91		1.276395

				268.93		1.276395

				268.95		1.276395

				268.97		1.276395

				268.99		1.276395

				269.01		1.276395

				269.03		1.276395

				269.05		1.276395

				269.07		1.276395

				269.09		1.276395

				269.11		1.276395

				269.13		1.272515

				269.15		1.272515

				269.18		1.272515

				269.2		1.272515

				269.22		1.272515

				269.24		1.272515

				269.26		1.272515

				269.28		1.272515

				269.3		1.272515

				269.32		1.272515

				269.34		1.272515

				269.36		1.272515

				269.38		1.272515

				269.4		1.272515

				269.43		1.272515

				269.45		1.272515

				269.47		1.272515

				269.49		1.272515

				269.51		1.272515

				269.53		1.268635

				269.55		1.268635

				269.57		1.268635

				269.59		1.264755

				269.61		1.264755

				269.63		1.264755

				269.65		1.264755

				269.67		1.264755

				269.7		1.260875

				269.72		1.260875

				269.74		1.260875

				269.76		1.260875

				269.78		1.260875

				269.8		1.260875

				269.82		1.260875

				269.84		1.260875

				269.86		1.260875

				269.88		1.256995

				269.9		1.256995

				269.92		1.256995

				269.94		1.256995

				269.97		1.256995

				269.99		1.253115

				270.01		1.253115

				270.03		1.253115

				270.05		1.253115

				270.07		1.253115

				270.09		1.249235

				270.11		1.249235

				270.13		1.249235

				270.15		1.249235

				270.17		1.249235

				270.19		1.249235

				270.21		1.245355

				270.24		1.249235

				270.26		1.245355

				270.28		1.245355

				270.3		1.245355

				270.32		1.245355

				270.34		1.245355

				270.36		1.245355

				270.38		1.241475

				270.4		1.241475

				270.42		1.241475

				270.44		1.241475

				270.46		1.237595

				270.48		1.237595

				270.51		1.237595

				270.53		1.237595

				270.55		1.233715

				270.57		1.233715

				270.59		1.233715

				270.61		1.233715

				270.63		1.233715

				270.65		1.233715

				270.67		1.233715

				270.69		1.233715

				270.71		1.233715

				270.73		1.233715

				270.76		1.233715

				270.78		1.229835

				270.8		1.229835

				270.82		1.233715

				270.84		1.229835

				270.86		1.229835

				270.88		1.229835

				270.9		1.229835

				270.92		1.229835

				270.94		1.229835

				270.96		1.229835

				270.98		1.225955

				271		1.225955

				271.03		1.225955

				271.05		1.225955

				271.07		1.225955

				271.09		1.225955

				271.11		1.225955

				271.13		1.225955

				271.15		1.225955

				271.17		1.222075

				271.19		1.222075

				271.21		1.222075

				271.23		1.222075

				271.25		1.222075

				271.28		1.222075

				271.3		1.222075

				271.32		1.222075

				271.34		1.222075

				271.36		1.222075

				271.38		1.218195

				271.4		1.222075

				271.42		1.218195

				271.44		1.218195

				271.46		1.218195

				271.48		1.218195

				271.5		1.218195

				271.52		1.218195

				271.55		1.214315

				271.57		1.218195

				271.59		1.214315

				271.61		1.214315

				271.63		1.214315

				271.65		1.214315

				271.67		1.214315

				271.69		1.214315

				271.71		1.214315

				271.73		1.214315

				271.75		1.214315

				271.77		1.214315

				271.8		1.214315

				271.82		1.210435

				271.84		1.210435

				271.86		1.210435

				271.88		1.210435

				271.9		1.210435

				271.92		1.210435

				271.94		1.210435

				271.96		1.210435

				271.98		1.210435

				272		1.210435

				272.02		1.210435

				272.04		1.210435

				272.07		1.206555

				272.09		1.206555

				272.11		1.210435

				272.13		1.206555

				272.15		1.206555

				272.17		1.206555

				272.19		1.206555

				272.21		1.206555

				272.23		1.206555

				272.25		1.206555

				272.27		1.206555

				272.29		1.202675

				272.32		1.206555

				272.34		1.206555

				272.36		1.206555

				272.38		1.202675

				272.4		1.202675

				272.42		1.202675

				272.44		1.202675

				272.46		1.202675

				272.48		1.202675

				272.5		1.202675

				272.52		1.202675

				272.54		1.202675

				272.56		1.202675

				272.59		1.202675

				272.61		1.202675

				272.63		1.202675

				272.65		1.198795

				272.67		1.198795

				272.69		1.198795

				272.71		1.198795

				272.73		1.198795

				272.75		1.198795

				272.77		1.198795

				272.79		1.198795

				272.81		1.198795

				272.83		1.198795

				272.86		1.198795

				272.88		1.198795

				272.9		1.198795

				272.92		1.198795

				272.94		1.198795

				272.96		1.198795

				272.98		1.198795

				273		1.198795

				273.02		1.198795

				273.04		1.198795

				273.06		1.198795

				273.08		1.198795

				273.11		1.198795

				273.13		1.198795

				273.15		1.198795

				273.17		1.198795

				273.19		1.198795

				273.21		1.198795

				273.23		1.194915

				273.25		1.194915

				273.27		1.194915

				273.29		1.194915

				273.31		1.194915

				273.33		1.194915

				273.35		1.194915

				273.38		1.194915

				273.4		1.194915

				273.42		1.194915

				273.44		1.194915

				273.46		1.194915

				273.48		1.194915

				273.5		1.194915

				273.52		1.194915

				273.54		1.194915

				273.56		1.194915

				273.58		1.194915

				273.6		1.194915

				273.63		1.194915

				273.65		1.194915

				273.67		1.194915

				273.69		1.194915

				273.71		1.194915

				273.73		1.194915

				273.75		1.194915

				273.77		1.194915

				273.79		1.194915

				273.81		1.194915

				273.83		1.194915

				273.85		1.194915

				273.88		1.194915

				273.9		1.194915

				273.92		1.194915

				273.94		1.194915

				273.96		1.194915

				273.98		1.194915

				274		1.191034

				274.02		1.191034

				274.04		1.191034

				274.06		1.194915

				274.08		1.191034

				274.1		1.191034

				274.13		1.191034

				274.15		1.191034

				274.17		1.191034

				274.19		1.191034

				274.21		1.191034

				274.23		1.191034

				274.25		1.191034

				274.27		1.191034

				274.29		1.191034

				274.31		1.191034

				274.33		1.191034

				274.35		1.191034

				274.38		1.191034

				274.4		1.191034

				274.42		1.191034

				274.44		1.191034

				274.46		1.191034

				274.48		1.191034

				274.5		1.191034

				274.52		1.187154

				274.54		1.187154

				274.56		1.187154

				274.58		1.187154

				274.6		1.191034

				274.63		1.187154

				274.65		1.187154

				274.67		1.187154

				274.69		1.187154

				274.71		1.187154

				274.73		1.187154

				274.75		1.187154

				274.77		1.187154

				274.79		1.187154

				274.81		1.187154

				274.83		1.187154

				274.85		1.187154

				274.88		1.187154

				274.9		1.187154

				274.92		1.187154

				274.94		1.183274

				274.96		1.183274

				274.98		1.183274

				275		1.183274

				275.02		1.183274

				275.04		1.183274

				275.06		1.183274

				275.08		1.179394

				275.1		1.179394

				275.13		1.179394

				275.15		1.179394

				275.17		1.179394

				275.19		1.179394

				275.21		1.179394

				275.23		1.179394

				275.25		1.179394

				275.27		1.175514

				275.29		1.175514

				275.31		1.175514

				275.33		1.175514

				275.35		1.175514

				275.38		1.175514

				275.4		1.175514

				275.42		1.175514

				275.44		1.171634

				275.46		1.171634

				275.48		1.171634

				275.5		1.171634

				275.52		1.171634

				275.54		1.171634

				275.56		1.171634

				275.58		1.171634

				275.6		1.167754

				275.63		1.167754

				275.65		1.167754

				275.67		1.167754

				275.69		1.167754

				275.71		1.167754

				275.73		1.167754

				275.75		1.167754

				275.77		1.167754

				275.79		1.163874

				275.81		1.163874

				275.83		1.163874

				275.86		1.163874

				275.88		1.163874

				275.9		1.163874

				275.92		1.163874

				275.94		1.163874

				275.96		1.163874

				275.98		1.159994

				276		1.159994

				276.02		1.159994

				276.04		1.159994

				276.06		1.159994

				276.09		1.159994

				276.11		1.159994

				276.13		1.159994

				276.15		1.156114

				276.17		1.156114

				276.19		1.156114

				276.21		1.156114

				276.23		1.156114

				276.25		1.156114

				276.27		1.156114

				276.29		1.156114

				276.31		1.156114

				276.34		1.156114

				276.36		1.156114

				276.38		1.156114

				276.4		1.156114

				276.42		1.156114

				276.44		1.152234

				276.46		1.152234

				276.48		1.152234

				276.5		1.152234

				276.52		1.152234

				276.54		1.152234

				276.57		1.152234

				276.59		1.152234

				276.61		1.152234

				276.63		1.152234

				276.65		1.152234

				276.67		1.148354

				276.69		1.152234

				276.71		1.152234

				276.73		1.148354

				276.75		1.148354

				276.77		1.148354

				276.79		1.148354

				276.82		1.148354

				276.84		1.148354

				276.86		1.148354

				276.88		1.148354

				276.9		1.148354

				276.92		1.148354

				276.94		1.148354

				276.96		1.148354

				276.98		1.144474

				277		1.144474

				277.02		1.144474

				277.04		1.144474

				277.07		1.144474

				277.09		1.144474

				277.11		1.144474

				277.13		1.144474

				277.15		1.144474

				277.17		1.144474

				277.19		1.144474

				277.21		1.144474

				277.23		1.144474

				277.25		1.144474

				277.27		1.144474

				277.3		1.144474

				277.32		1.144474

				277.34		1.144474

				277.36		1.144474

				277.38		1.144474

				277.4		1.144474

				277.42		1.144474

				277.44		1.144474

				277.46		1.144474

				277.48		1.144474

				277.5		1.144474

				277.53		1.144474

				277.55		1.144474

				277.57		1.140594

				277.59		1.140594

				277.61		1.140594

				277.63		1.140594

				277.65		1.140594

				277.67		1.140594

				277.69		1.140594

				277.71		1.140594

				277.73		1.140594

				277.75		1.140594

				277.78		1.140594

				277.8		1.140594

				277.82		1.140594

				277.84		1.140594

				277.86		1.140594

				277.88		1.140594

				277.9		1.140594

				277.92		1.140594

				277.94		1.140594

				277.96		1.140594

				277.98		1.140594

				278.01		1.140594

				278.03		1.140594

				278.05		1.140594

				278.07		1.140594

				278.09		1.140594

				278.11		1.140594

				278.13		1.140594

				278.15		1.140594

				278.17		1.140594

				278.19		1.140594

				278.21		1.140594

				278.24		1.140594

				278.26		1.140594

				278.28		1.136714

				278.3		1.136714

				278.32		1.136714

				278.34		1.136714

				278.36		1.136714

				278.38		1.136714

				278.4		1.136714

				278.42		1.136714

				278.44		1.136714

				278.46		1.136714

				278.49		1.136714

				278.51		1.136714

				278.53		1.136714

				278.55		1.136714

				278.57		1.136714

				278.59		1.136714

				278.61		1.136714

				278.63		1.136714

				278.65		1.136714

				278.67		1.136714

				278.69		1.136714

				278.72		1.136714

				278.74		1.136714

				278.76		1.136714

				278.78		1.132834

				278.8		1.132834

				278.82		1.132834

				278.84		1.132834

				278.86		1.132834

				278.88		1.132834

				278.9		1.132834

				278.92		1.132834

				278.95		1.132834

				278.97		1.132834

				278.99		1.132834

				279.01		1.132834

				279.03		1.132834

				279.05		1.128954

				279.07		1.128954

				279.09		1.128954

				279.11		1.128954

				279.13		1.128954

				279.15		1.128954

				279.17		1.128954

				279.2		1.128954

				279.22		1.128954

				279.24		1.128954

				279.26		1.128954

				279.28		1.128954

				279.3		1.128954

				279.32		1.128954

				279.34		1.128954

				279.36		1.128954

				279.38		1.128954

				279.4		1.128954

				279.43		1.128954

				279.45		1.128954

				279.47		1.128954

				279.49		1.128954

				279.51		1.128954

				279.53		1.128954

				279.55		1.128954

				279.57		1.128954

				279.59		1.128954

				279.61		1.128954

				279.63		1.128954

				279.66		1.128954

				279.68		1.128954

				279.7		1.128954

				279.72		1.128954

				279.74		1.128954

				279.76		1.128954

				279.78		1.128954

				279.8		1.128954

				279.82		1.128954

				279.84		1.128954

				279.86		1.128954

				279.88		1.128954

				279.91		1.125074

				279.93		1.125074

				279.95		1.125074

				279.97		1.125074

				279.99		1.125074

				280.01		1.125074

				280.03		1.125074

				280.05		1.125074

				280.07		1.125074

				280.09		1.125074

				280.11		1.125074

				280.14		1.125074

				280.16		1.125074

				280.18		1.125074

				280.2		1.125074

				280.22		1.125074

				280.24		1.125074

				280.26		1.125074

				280.28		1.125074

				280.3		1.125074

				280.32		1.125074

				280.34		1.125074

				280.36		1.125074

				280.39		1.125074

				280.41		1.125074

				280.43		1.125074

				280.45		1.125074

				280.47		1.125074

				280.49		1.125074

				280.51		1.125074

				280.53		1.125074

				280.55		1.125074

				280.57		1.125074

				280.59		1.125074

				280.62		1.125074

				280.64		1.125074

				280.66		1.125074

				280.68		1.125074

				280.7		1.121194

				280.72		1.121194

				280.74		1.121194

				280.76		1.121194

				280.78		1.121194

				280.8		1.121194

				280.82		1.121194

				280.85		1.121194

				280.87		1.121194

				280.89		1.121194

				280.91		1.121194

				280.93		1.121194

				280.95		1.121194

				280.97		1.121194

				280.99		1.121194

				281.01		1.121194

				281.03		1.121194

				281.05		1.121194

				281.08		1.121194

				281.1		1.125074

				281.12		1.125074

				281.14		1.125074

				281.16		1.125074

				281.18		1.125074

				281.2		1.125074

				281.22		1.125074

				281.24		1.125074

				281.26		1.125074

				281.28		1.125074

				281.31		1.125074

				281.33		1.125074

				281.35		1.125074

				281.37		1.125074

				281.39		1.121194

				281.41		1.121194

				281.43		1.121194

				281.45		1.121194

				281.47		1.121194

				281.49		1.121194

				281.51		1.125074

				281.54		1.121194

				281.56		1.125074

				281.58		1.121194

				281.6		1.121194

				281.62		1.121194

				281.64		1.121194

				281.66		1.125074

				281.68		1.121194

				281.7		1.121194

				281.72		1.121194

				281.75		1.121194

				281.77		1.121194

				281.79		1.121194

				281.81		1.121194

				281.83		1.121194

				281.85		1.121194

				281.87		1.121194

				281.89		1.121194

				281.91		1.121194

				281.93		1.121194

				281.95		1.121194

				281.98		1.121194

				282		1.121194

				282.02		1.121194

				282.04		1.121194

				282.06		1.121194

				282.08		1.121194

				282.1		1.121194

				282.12		1.121194

				282.14		1.121194

				282.16		1.121194

				282.18		1.121194

				282.21		1.121194

				282.23		1.121194

				282.25		1.121194

				282.27		1.121194

				282.29		1.121194

				282.31		1.121194

				282.33		1.121194

				282.35		1.121194

				282.37		1.121194

				282.39		1.121194

				282.41		1.121194

				282.44		1.121194

				282.46		1.121194

				282.48		1.121194

				282.5		1.121194

				282.52		1.121194

				282.54		1.121194

				282.56		1.121194

				282.58		1.121194

				282.6		1.121194

				282.62		1.121194

				282.64		1.121194

				282.67		1.121194

				282.69		1.121194

				282.71		1.121194

				282.73		1.121194

				282.75		1.121194

				282.77		1.121194

				282.79		1.121194

				282.81		1.121194

				282.83		1.121194

				282.85		1.121194

				282.87		1.121194

				282.9		1.121194

				282.92		1.121194

				282.94		1.121194

				282.96		1.121194

				282.98		1.121194

				283		1.117314

				283.02		1.117314

				283.04		1.117314

				283.06		1.121194

				283.08		1.117314

				283.1		1.121194

				283.13		1.117314

				283.15		1.117314

				283.17		1.117314

				283.19		1.117314

				283.21		1.117314

				283.23		1.117314

				283.25		1.117314

				283.27		1.117314

				283.29		1.117314

				283.31		1.117314

				283.33		1.117314

				283.36		1.117314

				283.38		1.113434

				283.4		1.113434

				283.42		1.117314

				283.44		1.113434

				283.46		1.113434

				283.48		1.117314

				283.5		1.113434

				283.52		1.113434

				283.54		1.113434

				283.56		1.113434

				283.59		1.113434

				283.61		1.113434

				283.63		1.113434

				283.65		1.113434

				283.67		1.113434

				283.69		1.113434

				283.71		1.113434

				283.73		1.109554

				283.75		1.109554

				283.77		1.109554

				283.79		1.109554

				283.82		1.109554

				283.84		1.109554

				283.86		1.109554

				283.88		1.109554

				283.9		1.109554

				283.92		1.109554

				283.94		1.109554

				283.96		1.105674

				283.98		1.105674

				284		1.105674

				284.02		1.105674

				284.05		1.105674

				284.07		1.105674

				284.09		1.105674

				284.11		1.105674

				284.13		1.105674

				284.15		1.105674

				284.17		1.105674

				284.19		1.101794

				284.21		1.101794

				284.23		1.101794

				284.25		1.101794

				284.28		1.101794

				284.3		1.101794

				284.32		1.101794

				284.34		1.101794

				284.36		1.101794

				284.38		1.097914

				284.4		1.101794

				284.42		1.097914

				284.44		1.097914

				284.46		1.097914

				284.48		1.097914

				284.51		1.097914

				284.53		1.097914

				284.55		1.097914

				284.57		1.097914

				284.59		1.097914

				284.61		1.097914

				284.63		1.097914

				284.65		1.097914

				284.67		1.097914

				284.69		1.097914

				284.71		1.097914

				284.74		1.097914

				284.76		1.097914

				284.78		1.097914

				284.8		1.097914

				284.82		1.097914

				284.84		1.097914

				284.86		1.097914

				284.88		1.097914

				284.9		1.097914

				284.92		1.097914

				284.94		1.094034

				284.97		1.097914

				284.99		1.094034

				285.01		1.094034

				285.03		1.094034

				285.05		1.094034

				285.07		1.094034

				285.09		1.094034

				285.11		1.094034

				285.13		1.094034

				285.15		1.094034

				285.18		1.094034

				285.2		1.094034

				285.22		1.094034

				285.24		1.094034

				285.26		1.094034

				285.28		1.094034

				285.3		1.094034

				285.32		1.094034

				285.34		1.094034

				285.36		1.094034

				285.38		1.094034

				285.41		1.094034

				285.43		1.094034

				285.45		1.094034

				285.47		1.094034

				285.49		1.090154

				285.51		1.090154

				285.53		1.090154

				285.55		1.090154

				285.57		1.090154

				285.59		1.090154

				285.61		1.094034

				285.64		1.090154

				285.66		1.090154

				285.68		1.090154

				285.7		1.090154

				285.72		1.090154

				285.74		1.090154

				285.76		1.090154

				285.78		1.090154

				285.8		1.090154

				285.82		1.090154

				285.84		1.090154

				285.87		1.090154

				285.89		1.090154

				285.91		1.090154

				285.93		1.090154

				285.95		1.090154

				285.97		1.090154

				285.99		1.090154

				286.01		1.094034

				286.03		1.094034

				286.05		1.094034

				286.08		1.094034

				286.1		1.090154

				286.12		1.090154

				286.14		1.090154

				286.16		1.094034

				286.18		1.094034

				286.2		1.094034

				286.22		1.094034

				286.24		1.094034

				286.26		1.094034

				286.28		1.094034

				286.31		1.094034

				286.33		1.094034

				286.35		1.094034

				286.37		1.094034

				286.39		1.094034

				286.41		1.094034

				286.43		1.094034

				286.45		1.094034

				286.47		1.094034

				286.49		1.094034

				286.51		1.094034

				286.54		1.094034

				286.56		1.094034

				286.58		1.094034

				286.6		1.094034

				286.62		1.094034

				286.64		1.094034

				286.66		1.094034

				286.68		1.094034

				286.7		1.094034

				286.72		1.094034

				286.74		1.090154

				286.77		1.094034

				286.79		1.094034

				286.81		1.090154

				286.83		1.090154

				286.85		1.094034

				286.87		1.094034

				286.89		1.090154

				286.91		1.090154

				286.93		1.090154

				286.95		1.090154

				286.97		1.090154

				287		1.090154

				287.02		1.090154

				287.04		1.090154

				287.06		1.090154

				287.08		1.090154

				287.1		1.090154

				287.12		1.090154

				287.14		1.090154

				287.16		1.090154

				287.18		1.090154

				287.2		1.090154

				287.23		1.094034

				287.25		1.090154

				287.27		1.090154

				287.29		1.090154

				287.31		1.090154

				287.33		1.090154

				287.35		1.090154

				287.37		1.090154

				287.39		1.090154

				287.41		1.090154

				287.44		1.090154

				287.46		1.090154

				287.48		1.090154

				287.5		1.090154

				287.52		1.090154

				287.54		1.090154

				287.56		1.090154

				287.58		1.090154

				287.6		1.090154

				287.62		1.086274

				287.64		1.086274

				287.67		1.090154

				287.69		1.086274

				287.71		1.086274

				287.73		1.090154

				287.75		1.086274

				287.77		1.086274

				287.79		1.086274

				287.81		1.086274

				287.83		1.086274

				287.85		1.090154

				287.88		1.090154

				287.9		1.090154

				287.92		1.090154

				287.94		1.090154

				287.96		1.090154

				287.98		1.090154

				288		1.090154

				288.02		1.090154

				288.04		1.090154

				288.06		1.090154

				288.08		1.090154

				288.11		1.086274

				288.13		1.086274

				288.15		1.090154

				288.17		1.086274

				288.19		1.086274

				288.21		1.086274

				288.23		1.086274

				288.25		1.086274

				288.27		1.086274

				288.29		1.086274

				288.32		1.086274

				288.34		1.086274

				288.36		1.086274

				288.38		1.086274

				288.4		1.086274

				288.42		1.086274

				288.44		1.086274

				288.46		1.086274

				288.48		1.086274

				288.5		1.086274

				288.52		1.086274

				288.55		1.086274

				288.57		1.086274

				288.59		1.086274

				288.61		1.086274

				288.63		1.086274

				288.65		1.086274

				288.67		1.086274

				288.69		1.086274

				288.71		1.086274

				288.73		1.086274

				288.76		1.086274

				288.78		1.086274

				288.8		1.086274

				288.82		1.086274

				288.84		1.086274

				288.86		1.086274

				288.88		1.086274

				288.9		1.086274

				288.92		1.086274

				288.94		1.086274

				288.97		1.086274

				288.99		1.086274

				289.01		1.086274

				289.03		1.082393

				289.05		1.086274

				289.07		1.082393

				289.09		1.082393

				289.11		1.082393

				289.13		1.082393

				289.15		1.082393

				289.17		1.082393

				289.2		1.082393

				289.22		1.082393

				289.24		1.082393

				289.26		1.082393

				289.28		1.082393

				289.3		1.082393

				289.32		1.082393

				289.34		1.082393

				289.36		1.082393

				289.38		1.082393

				289.41		1.082393

				289.43		1.082393

				289.45		1.082393

				289.47		1.082393

				289.49		1.082393

				289.51		1.082393

				289.53		1.082393

				289.55		1.082393

				289.57		1.082393

				289.59		1.082393

				289.62		1.082393

				289.64		1.082393

				289.66		1.082393

				289.68		1.078513

				289.7		1.082393

				289.72		1.082393

				289.74		1.078513

				289.76		1.078513

				289.78		1.078513

				289.8		1.078513

				289.83		1.078513

				289.85		1.082393

				289.87		1.078513

				289.89		1.082393

				289.91		1.078513

				289.93		1.078513

				289.95		1.078513

				289.97		1.078513

				289.99		1.078513

				290.01		1.078513

				290.04		1.078513

				290.06		1.078513

				290.08		1.078513

				290.1		1.078513

				290.12		1.078513

				290.14		1.074633

				290.16		1.074633

				290.18		1.078513

				290.2		1.078513

				290.22		1.078513

				290.25		1.078513

				290.27		1.078513

				290.29		1.078513

				290.31		1.078513

				290.33		1.078513

				290.35		1.078513

				290.37		1.078513

				290.39		1.074633

				290.41		1.074633

				290.43		1.074633

				290.46		1.074633

				290.48		1.074633

				290.5		1.074633

				290.52		1.074633

				290.54		1.074633

				290.56		1.074633

				290.58		1.074633

				290.6		1.074633

				290.62		1.074633

				290.64		1.074633

				290.67		1.074633

				290.69		1.074633

				290.71		1.074633

				290.73		1.074633

				290.75		1.074633

				290.77		1.074633

				290.79		1.074633

				290.81		1.074633

				290.83		1.074633

				290.85		1.074633

				290.88		1.074633

				290.9		1.074633

				290.92		1.074633

				290.94		1.074633

				290.96		1.070753

				290.98		1.074633

				291		1.070753

				291.02		1.070753

				291.04		1.070753

				291.06		1.070753

				291.09		1.074633

				291.11		1.074633

				291.13		1.074633

				291.15		1.074633

				291.17		1.074633

				291.19		1.074633

				291.21		1.074633

				291.23		1.074633

				291.25		1.074633

				291.27		1.074633

				291.3		1.074633

				291.32		1.074633

				291.34		1.074633

				291.36		1.074633

				291.38		1.074633

				291.4		1.074633

				291.42		1.074633

				291.44		1.074633

				291.46		1.074633

				291.48		1.074633

				291.51		1.074633

				291.53		1.074633

				291.55		1.074633

				291.57		1.074633

				291.59		1.074633

				291.61		1.074633

				291.63		1.074633

				291.65		1.074633

				291.67		1.074633

				291.69		1.074633

				291.72		1.074633

				291.74		1.074633

				291.76		1.074633

				291.78		1.074633

				291.8		1.074633

				291.82		1.074633

				291.84		1.074633

				291.86		1.074633

				291.88		1.074633

				291.9		1.070753

				291.93		1.070753

				291.95		1.070753

				291.97		1.070753

				291.99		1.070753

				292.01		1.070753

				292.03		1.070753

				292.05		1.070753

				292.07		1.070753

				292.09		1.070753

				292.11		1.070753

				292.14		1.070753

				292.16		1.070753

				292.18		1.070753

				292.2		1.070753

				292.22		1.070753

				292.24		1.070753

				292.26		1.070753

				292.28		1.070753

				292.3		1.070753

				292.32		1.070753

				292.35		1.070753

				292.37		1.070753

				292.39		1.066873

				292.41		1.066873

				292.43		1.066873

				292.45		1.066873

				292.47		1.066873

				292.49		1.066873

				292.51		1.066873

				292.53		1.066873

				292.56		1.070753

				292.58		1.066873

				292.6		1.066873

				292.62		1.066873

				292.64		1.066873

				292.66		1.066873

				292.68		1.066873

				292.7		1.066873

				292.72		1.066873

				292.74		1.066873

				292.77		1.066873

				292.79		1.066873

				292.81		1.066873

				292.83		1.066873

				292.85		1.066873

				292.87		1.066873

				292.89		1.066873

				292.91		1.062993

				292.93		1.062993

				292.95		1.062993

				292.98		1.062993

				293		1.062993

				293.02		1.062993

				293.04		1.062993

				293.06		1.062993

				293.08		1.062993

				293.1		1.062993

				293.12		1.062993

				293.14		1.062993

				293.16		1.062993

				293.19		1.062993

				293.21		1.062993

				293.23		1.062993

				293.25		1.062993

				293.27		1.062993

				293.29		1.062993

				293.31		1.062993

				293.33		1.062993

				293.35		1.059113

				293.38		1.059113

				293.4		1.059113

				293.42		1.059113

				293.44		1.059113

				293.46		1.059113

				293.48		1.059113

				293.5		1.059113

				293.52		1.059113

				293.54		1.059113

				293.56		1.059113

				293.59		1.059113

				293.61		1.059113

				293.63		1.059113

				293.65		1.059113

				293.67		1.059113

				293.69		1.059113

				293.71		1.059113

				293.73		1.059113

				293.75		1.059113

				293.77		1.059113

				293.8		1.059113

				293.82		1.059113

				293.84		1.059113

				293.86		1.059113

				293.88		1.055233

				293.9		1.055233

				293.92		1.055233

				293.94		1.055233

				293.96		1.055233

				293.98		1.055233

				294.01		1.055233

				294.03		1.059113

				294.05		1.055233

				294.07		1.055233

				294.09		1.055233

				294.11		1.055233

				294.13		1.055233

				294.15		1.055233

				294.17		1.055233

				294.2		1.055233

				294.22		1.055233

				294.24		1.055233

				294.26		1.055233

				294.28		1.055233

				294.3		1.055233

				294.32		1.055233

				294.34		1.055233

				294.36		1.055233

				294.38		1.055233

				294.41		1.055233

				294.43		1.055233

				294.45		1.055233

				294.47		1.055233

				294.49		1.055233

				294.51		1.055233

				294.53		1.055233

				294.55		1.055233

				294.57		1.055233

				294.59		1.055233

				294.62		1.055233

				294.64		1.055233

				294.66		1.055233

				294.68		1.055233

				294.7		1.055233

				294.72		1.055233

				294.74		1.055233

				294.76		1.055233

				294.78		1.055233

				294.81		1.055233

				294.83		1.055233

				294.85		1.055233

				294.87		1.055233

				294.89		1.055233

				294.91		1.055233

				294.93		1.055233

				294.95		1.055233

				294.97		1.055233

				294.99		1.055233

				295.02		1.055233

				295.04		1.055233

				295.06		1.055233

				295.08		1.055233

				295.1		1.055233

				295.12		1.055233

				295.14		1.055233

				295.16		1.055233

				295.18		1.055233

				295.21		1.055233

				295.23		1.055233

				295.25		1.055233

				295.27		1.055233

				295.29		1.055233

				295.31		1.055233

				295.33		1.055233

				295.35		1.051353

				295.37		1.055233

				295.39		1.055233

				295.42		1.055233

				295.44		1.055233

				295.46		1.055233

				295.48		1.055233

				295.5		1.055233

				295.52		1.055233

				295.54		1.055233

				295.56		1.055233

				295.58		1.055233

				295.61		1.055233

				295.63		1.055233

				295.65		1.055233

				295.67		1.055233

				295.69		1.055233

				295.71		1.055233

				295.73		1.055233

				295.75		1.055233

				295.77		1.055233

				295.8		1.055233

				295.82		1.055233

				295.84		1.055233

				295.86		1.055233

				295.88		1.055233

				295.9		1.055233

				295.92		1.055233

				295.94		1.055233

				295.96		1.055233

				295.99		1.055233

				296.01		1.055233

				296.03		1.055233

				296.05		1.055233

				296.07		1.055233

				296.09		1.055233

				296.11		1.055233

				296.13		1.055233

				296.15		1.055233

				296.17		1.055233

				296.2		1.055233

				296.22		1.055233

				296.24		1.055233

				296.26		1.055233

				296.28		1.055233

				296.3		1.055233

				296.32		1.055233

				296.34		1.055233

				296.36		1.055233

				296.39		1.051353

				296.41		1.051353

				296.43		1.051353

				296.45		1.055233

				296.47		1.051353

				296.49		1.055233

				296.51		1.055233

				296.53		1.055233

				296.55		1.055233

				296.58		1.055233

				296.6		1.055233

				296.62		1.055233

				296.64		1.055233

				296.66		1.055233

				296.68		1.055233

				296.7		1.055233

				296.72		1.055233

				296.74		1.055233

				296.76		1.055233

				296.79		1.055233

				296.81		1.055233

				296.83		1.055233

				296.85		1.055233

				296.87		1.055233

				296.89		1.055233

				296.91		1.055233

				296.93		1.055233

				296.95		1.055233

				296.98		1.055233

				297		1.055233

				297.02		1.055233

				297.04		1.055233

				297.06		1.055233

				297.08		1.055233

				297.1		1.055233

				297.12		1.055233

				297.14		1.055233

				297.17		1.055233

				297.19		1.055233

				297.21		1.055233

				297.23		1.055233

				297.25		1.055233

				297.27		1.055233

				297.29		1.055233

				297.31		1.055233

				297.33		1.055233

				297.35		1.055233

				297.38		1.055233

				297.4		1.055233

				297.42		1.055233

				297.44		1.055233

				297.46		1.055233

				297.48		1.055233

				297.5		1.055233

				297.52		1.055233

				297.54		1.055233

				297.57		1.055233

				297.59		1.055233

				297.61		1.055233

				297.63		1.055233

				297.65		1.055233

				297.67		1.055233

				297.69		1.055233

				297.71		1.055233

				297.73		1.055233

				297.75		1.055233

				297.78		1.051353

				297.8		1.055233

				297.82		1.051353

				297.84		1.055233

				297.86		1.051353

				297.88		1.051353

				297.9		1.055233

				297.92		1.051353

				297.94		1.051353

				297.97		1.055233

				297.99		1.051353

				298.01		1.051353

				298.03		1.055233

				298.05		1.051353

				298.07		1.055233

				298.09		1.055233

				298.11		1.055233

				298.13		1.051353

				298.16		1.051353

				298.18		1.055233

				298.2		1.051353

				298.22		1.051353

				298.24		1.051353

				298.26		1.055233

				298.28		1.051353

				298.3		1.055233

				298.32		1.055233

				298.34		1.055233

				298.37		1.055233

				298.39		1.051353

				298.41		1.051353

				298.43		1.051353

				298.45		1.055233

				298.47		1.055233

				298.49		1.055233

				298.51		1.055233

				298.53		1.051353

				298.56		1.051353

				298.58		1.051353

				298.6		1.051353

				298.62		1.051353

				298.64		1.051353

				298.66		1.051353

				298.68		1.051353

				298.7		1.051353

				298.72		1.051353

				298.74		1.051353

				298.77		1.051353

				298.79		1.051353

				298.81		1.051353

				298.83		1.051353

				298.85		1.051353

				298.87		1.051353

				298.89		1.051353

				298.91		1.051353

				298.93		1.051353

				298.96		1.051353

				298.98		1.051353

				299		1.051353

				299.02		1.051353

				299.04		1.051353

				299.06		1.051353

				299.08		1.051353

				299.1		1.051353

				299.12		1.051353

				299.14		1.051353

				299.17		1.051353

				299.19		1.051353

				299.21		1.051353

				299.23		1.051353

				299.25		1.051353

				299.27		1.047473

				299.29		1.047473

				299.31		1.047473

				299.33		1.047473

				299.36		1.047473

				299.38		1.047473

				299.4		1.047473

				299.42		1.047473

				299.44		1.047473

				299.46		1.047473

				299.48		1.047473

				299.5		1.047473

				299.52		1.047473

				299.54		1.047473

				299.57		1.047473

				299.59		1.047473

				299.61		1.047473

				299.63		1.047473

				299.65		1.047473

				299.67		1.047473

				299.69		1.047473

				299.71		1.047473

				299.73		1.047473

				299.76		1.047473

				299.78		1.047473

				299.8		1.047473

				299.82		1.047473

				299.84		1.047473

				299.86		1.047473

				299.88		1.047473

				299.9		1.047473

				299.92		1.047473

				299.95		1.047473

				299.97		1.047473

				299.99		1.047473

				300.01		1.047473

				300.03		1.047473

				300.05		1.047473

				300.07		1.047473

				300.09		1.047473

				300.11		1.047473

				300.13		1.047473

				300.16		1.047473

				300.18		1.043593

				300.2		1.043593

				300.22		1.043593

				300.24		1.043593

				300.26		1.043593

				300.28		1.043593

				300.3		1.043593

				300.32		1.043593

				300.35		1.043593

				300.37		1.043593

				300.39		1.043593

				300.41		1.043593

				300.43		1.043593

				300.45		1.043593

				300.47		1.043593

				300.49		1.043593

				300.51		1.043593

				300.54		1.043593

				300.56		1.043593

				300.58		1.043593

				300.6		1.043593

				300.62		1.043593

				300.64		1.043593

				300.66		1.043593

				300.68		1.043593

				300.7		1.043593

				300.72		1.043593

				300.75		1.043593

				300.77		1.043593

				300.79		1.043593

				300.81		1.043593

				300.83		1.043593

				300.85		1.043593

				300.87		1.043593

				300.89		1.043593

				300.91		1.043593

				300.94		1.039713

				300.96		1.039713

				300.98		1.039713

				301		1.039713

				301.02		1.039713

				301.04		1.039713

				301.06		1.039713

				301.08		1.039713

				301.1		1.039713

				301.13		1.039713

				301.15		1.039713

				301.17		1.039713

				301.19		1.035833

				301.21		1.039713

				301.23		1.035833

				301.25		1.039713

				301.27		1.039713

				301.29		1.035833

				301.32		1.035833

				301.34		1.035833

				301.36		1.035833

				301.38		1.035833

				301.4		1.035833

				301.42		1.035833

				301.44		1.035833

				301.46		1.035833

				301.48		1.035833

				301.51		1.035833

				301.53		1.035833

				301.55		1.035833

				301.57		1.035833

				301.59		1.035833

				301.61		1.035833

				301.63		1.035833

				301.65		1.035833

				301.67		1.035833

				301.69		1.035833

				301.72		1.031953

				301.74		1.031953

				301.76		1.031953

				301.78		1.031953

				301.8		1.031953

				301.82		1.031953

				301.84		1.031953

				301.86		1.031953

				301.88		1.031953

				301.91		1.031953

				301.93		1.031953

				301.95		1.031953

				301.97		1.031953

				301.99		1.031953

				302.01		1.031953

				302.03		1.031953

				302.05		1.031953

				302.07		1.031953

				302.1		1.031953

				302.12		1.031953

				302.14		1.031953

				302.16		1.031953

				302.18		1.031953

				302.2		1.031953

				302.22		1.031953

				302.24		1.031953

				302.26		1.031953

				302.28		1.031953

				302.31		1.031953

				302.33		1.031953

				302.35		1.031953

				302.37		1.031953

				302.39		1.028073

				302.41		1.028073

				302.43		1.028073

				302.45		1.028073

				302.47		1.028073

				302.5		1.028073

				302.52		1.028073

				302.54		1.028073

				302.56		1.028073

				302.58		1.028073

				302.6		1.028073

				302.62		1.028073

				302.64		1.028073

				302.66		1.028073

				302.69		1.028073

				302.71		1.028073

				302.73		1.028073

				302.75		1.028073

				302.77		1.028073

				302.79		1.024193

				302.81		1.024193

				302.83		1.028073

				302.85		1.024193

				302.87		1.024193

				302.9		1.028073

				302.92		1.024193

				302.94		1.024193

				302.96		1.024193

				302.98		1.024193

				303		1.024193

				303.02		1.024193

				303.04		1.024193

				303.06		1.024193

				303.09		1.024193

				303.11		1.024193

				303.13		1.024193

				303.15		1.024193

				303.17		1.024193

				303.19		1.024193

				303.21		1.024193

				303.23		1.024193

				303.25		1.024193

				303.28		1.024193

				303.3		1.024193

				303.32		1.024193

				303.34		1.024193

				303.36		1.024193

				303.38		1.024193

				303.4		1.024193

				303.42		1.024193

				303.44		1.024193

				303.46		1.024193

				303.49		1.024193

				303.51		1.024193

				303.53		1.024193

				303.55		1.024193

				303.57		1.024193

				303.59		1.024193

				303.61		1.024193

				303.63		1.024193

				303.65		1.024193

				303.68		1.024193

				303.7		1.028073

				303.72		1.028073

				303.74		1.028073

				303.76		1.028073

				303.78		1.028073

				303.8		1.028073

				303.82		1.028073

				303.84		1.028073

				303.87		1.028073

				303.89		1.028073

				303.91		1.028073

				303.93		1.028073

				303.95		1.028073

				303.97		1.028073

				303.99		1.028073

				304.01		1.028073

				304.03		1.028073

				304.06		1.024193

				304.08		1.024193

				304.1		1.028073

				304.12		1.031953

				304.14		1.031953

				304.16		1.028073

				304.18		1.028073

				304.2		1.031953

				304.22		1.031953

				304.25		1.031953

				304.27		1.031953

				304.29		1.031953

				304.31		1.031953

				304.33		1.031953

				304.35		1.031953

				304.37		1.031953

				304.39		1.031953

				304.41		1.031953

				304.44		1.031953

				304.46		1.031953

				304.48		1.031953

				304.5		1.031953

				304.52		1.031953

				304.54		1.031953

				304.56		1.031953

				304.58		1.031953

				304.6		1.031953

				304.63		1.031953

				304.65		1.031953

				304.67		1.031953

				304.69		1.031953

				304.71		1.031953

				304.73		1.031953

				304.75		1.031953

				304.77		1.031953

				304.79		1.031953

				304.81		1.031953

				304.84		1.031953

				304.86		1.035833

				304.88		1.031953

				304.9		1.031953

				304.92		1.031953

				304.94		1.035833

				304.96		1.035833

				304.98		1.031953

				305		1.035833

				305.03		1.035833

				305.05		1.035833

				305.07		1.035833

				305.09		1.035833

				305.11		1.035833

				305.13		1.035833

				305.15		1.035833

				305.17		1.035833

				305.19		1.039713

				305.22		1.035833

				305.24		1.039713

				305.26		1.039713

				305.28		1.035833

				305.3		1.035833

				305.32		1.035833

				305.34		1.035833

				305.36		1.035833

				305.38		1.035833

				305.41		1.035833

				305.43		1.035833

				305.45		1.035833

				305.47		1.035833

				305.49		1.035833

				305.51		1.035833

				305.53		1.035833

				305.55		1.035833

				305.57		1.035833

				305.6		1.035833

				305.62		1.035833

				305.64		1.035833

				305.66		1.035833

				305.68		1.035833

				305.7		1.039713

				305.72		1.035833

				305.74		1.035833

				305.76		1.035833

				305.79		1.035833

				305.81		1.035833

				305.83		1.035833

				305.85		1.035833

				305.87		1.035833

				305.89		1.035833

				305.91		1.035833

				305.93		1.035833

				305.95		1.035833

				305.98		1.035833

				306		1.035833

				306.02		1.035833

				306.04		1.035833

				306.06		1.035833

				306.08		1.035833

				306.1		1.035833

				306.12		1.035833

				306.14		1.039713

				306.17		1.039713

				306.19		1.035833

				306.21		1.031953

				306.23		1.031953

				306.25		1.035833

				306.27		1.035833

				306.29		1.035833

				306.31		1.035833

				306.33		1.035833

				306.36		1.031953

				306.38		1.035833

				306.4		1.031953

				306.42		1.035833

				306.44		1.031953

				306.46		1.031953

				306.48		1.031953

				306.5		1.031953

				306.52		1.031953

				306.55		1.031953

				306.57		1.031953

				306.59		1.031953

				306.61		1.031953

				306.63		1.035833

				306.65		1.035833

				306.67		1.035833

				306.69		1.035833

				306.71		1.031953

				306.73		1.031953

				306.76		1.031953

				306.78		1.031953

				306.8		1.031953

				306.82		1.031953

				306.84		1.035833

				306.86		1.031953

				306.88		1.031953

				306.9		1.031953

				306.92		1.031953

				306.95		1.031953

				306.97		1.031953

				306.99		1.031953

				307.01		1.031953

				307.03		1.031953

				307.05		1.031953

				307.07		1.031953

				307.09		1.031953

				307.11		1.031953

				307.14		1.031953

				307.16		1.031953

				307.18		1.031953

				307.2		1.031953

				307.22		1.031953

				307.24		1.031953

				307.26		1.031953

				307.28		1.028073

				307.3		1.028073

				307.32		1.028073

				307.35		1.028073

				307.37		1.028073

				307.39		1.028073

				307.41		1.031953

				307.43		1.028073

				307.45		1.031953

				307.47		1.028073

				307.49		1.031953

				307.51		1.028073

				307.54		1.028073

				307.56		1.028073

				307.58		1.028073

				307.6		1.028073

				307.62		1.028073

				307.64		1.028073

				307.66		1.028073

				307.68		1.028073

				307.7		1.028073

				307.73		1.028073

				307.75		1.028073

				307.77		1.028073

				307.79		1.028073

				307.81		1.028073

				307.83		1.028073

				307.85		1.028073

				307.87		1.028073

				307.89		1.028073

				307.92		1.028073

				307.94		1.024193

				307.96		1.028073

				307.98		1.028073

				308		1.024193

				308.02		1.024193

				308.04		1.024193

				308.06		1.024193

				308.08		1.024193

				308.11		1.024193

				308.13		1.024193

				308.15		1.024193

				308.17		1.024193

				308.19		1.024193

				308.21		1.024193

				308.23		1.024193

				308.25		1.024193

				308.27		1.024193

				308.3		1.024193

				308.32		1.024193

				308.34		1.024193

				308.36		1.024193

				308.38		1.024193

				308.4		1.024193

				308.42		1.024193

				308.44		1.024193

				308.46		1.024193

				308.49		1.024193

				308.51		1.024193

				308.53		1.024193

				308.55		1.024193

				308.57		1.024193

				308.59		1.024193

				308.61		1.024193

				308.63		1.024193

				308.65		1.024193

				308.68		1.024193

				308.7		1.024193

				308.72		1.024193

				308.74		1.024193

				308.76		1.024193

				308.78		1.024193

				308.8		1.024193

				308.82		1.024193

				308.84		1.024193

				308.87		1.024193

				308.89		1.024193

				308.91		1.024193

				308.93		1.024193

				308.95		1.024193

				308.97		1.024193

				308.99		1.024193

				309.01		1.024193

				309.03		1.024193

				309.06		1.028073

				309.08		1.024193

				309.1		1.024193

				309.12		1.024193

				309.14		1.024193

				309.16		1.024193

				309.18		1.024193

				309.2		1.024193

				309.22		1.028073

				309.25		1.024193

				309.27		1.024193

				309.29		1.024193

				309.31		1.028073

				309.33		1.024193

				309.35		1.028073

				309.37		1.028073

				309.39		1.024193

				309.41		1.024193

				309.44		1.024193

				309.46		1.024193

				309.48		1.024193

				309.5		1.024193

				309.52		1.024193

				309.54		1.024193

				309.56		1.028073

				309.58		1.024193

				309.61		1.024193

				309.63		1.024193

				309.65		1.024193

				309.67		1.024193

				309.69		1.024193

				309.71		1.028073

				309.73		1.028073

				309.75		1.028073

				309.77		1.028073

				309.8		1.028073

				309.82		1.028073

				309.84		1.028073

				309.86		1.028073

				309.88		1.024193

				309.9		1.028073

				309.92		1.024193

				309.94		1.024193

				309.96		1.028073

				309.99		1.028073

				310.01		1.024193

				310.03		1.028073

				310.05		1.028073

				310.07		1.028073

				310.09		1.028073

				310.11		1.028073

				310.13		1.028073

				310.15		1.028073

				310.18		1.028073

				310.2		1.028073

				310.22		1.028073

				310.24		1.028073

				310.26		1.028073

				310.28		1.028073

				310.3		1.028073

				310.32		1.028073

				310.34		1.028073

				310.37		1.028073

				310.39		1.028073

				310.41		1.028073

				310.43		1.028073

				310.45		1.028073

				310.47		1.028073

				310.49		1.028073

				310.51		1.028073

				310.53		1.028073

				310.56		1.028073

				310.58		1.028073

				310.6		1.028073

				310.62		1.028073

				310.64		1.028073

				310.66		1.028073

				310.68		1.024193

				310.7		1.028073

				310.72		1.024193

				310.75		1.024193

				310.77		1.024193

				310.79		1.024193

				310.81		1.024193

				310.83		1.024193

				310.85		1.024193

				310.87		1.024193

				310.89		1.024193

				310.91		1.024193

				310.94		1.024193

				310.96		1.024193

				310.98		1.024193

				311		1.024193

				311.02		1.024193

				311.04		1.024193

				311.06		1.024193

				311.08		1.024193

				311.1		1.024193

				311.13		1.024193

				311.15		1.020313

				311.17		1.020313

				311.19		1.020313

				311.21		1.020313

				311.23		1.020313

				311.25		1.020313

				311.27		1.020313

				311.29		1.020313

				311.32		1.020313

				311.34		1.020313

				311.36		1.020313

				311.38		1.020313

				311.4		1.020313

				311.42		1.020313

				311.44		1.020313

				311.46		1.020313

				311.48		1.020313

				311.51		1.020313

				311.53		1.020313

				311.55		1.016433

				311.57		1.016433

				311.59		1.020313

				311.61		1.016433

				311.63		1.016433

				311.65		1.016433

				311.67		1.016433

				311.7		1.016433

				311.72		1.016433

				311.74		1.016433

				311.76		1.016433

				311.78		1.016433

				311.8		1.016433

				311.82		1.016433

				311.84		1.016433

				311.86		1.012553

				311.89		1.012553

				311.91		1.012553

				311.93		1.012553

				311.95		1.012553

				311.97		1.012553

				311.99		1.012553

				312.01		1.012553

				312.03		1.012553

				312.05		1.012553

				312.08		1.012553

				312.1		1.012553

				312.12		1.012553

				312.14		1.012553

				312.16		1.012553

				312.18		1.012553

				312.2		1.012553

				312.22		1.012553

				312.24		1.012553

				312.27		1.012553

				312.29		1.012553

				312.31		1.008673

				312.33		1.008673

				312.35		1.008673

				312.37		1.008673

				312.39		1.008673

				312.41		1.008673

				312.43		1.008673

				312.46		1.008673

				312.48		1.008673

				312.5		1.008673

				312.52		1.008673

				312.54		1.008673

				312.56		1.008673

				312.58		1.008673

				312.6		1.008673

				312.62		1.008673

				312.65		1.008673

				312.67		1.008673

				312.69		1.008673

				312.71		1.008673

				312.73		1.008673

				312.75		1.008673

				312.77		1.008673

				312.79		1.008673

				312.81		1.008673

				312.84		1.008673

				312.86		1.008673

				312.88		1.008673

				312.9		1.008673

				312.92		1.008673

				312.94		1.008673

				312.96		1.008673

				312.98		1.008673

				313		1.008673

				313.03		1.008673

				313.05		1.008673

				313.07		1.008673

				313.09		1.008673

				313.11		1.008673

				313.13		1.008673

				313.15		1.008673

				313.17		1.008673

				313.2		1.008673

				313.22		1.008673

				313.24		1.008673

				313.26		1.008673

				313.28		1.008673

				313.3		1.008673

				313.32		1.008673

				313.34		1.008673

				313.36		1.008673

				313.39		1.008673

				313.41		1.008673

				313.43		1.008673

				313.45		1.008673

				313.47		1.008673

				313.49		1.008673

				313.51		1.008673

				313.53		1.008673

				313.55		1.008673

				313.58		1.008673

				313.6		1.008673

				313.62		1.008673

				313.64		1.008673

				313.66		1.008673

				313.68		1.008673

				313.7		1.008673

				313.72		1.008673

				313.74		1.008673

				313.77		1.004793

				313.79		1.004793

				313.81		1.004793

				313.83		1.004793

				313.85		1.004793

				313.87		1.004793

				313.89		1.004793

				313.91		1.004793

				313.93		1.004793

				313.96		1.004793

				313.98		1.004793

				314		1.004793

				314.02		1.004793

				314.04		1.004793

				314.06		1.004793

				314.08		1.004793

				314.1		1.004793

				314.12		1.004793

				314.15		1.004793

				314.17		1.004793

				314.19		1.004793

				314.21		1.004793

				314.23		1.004793

				314.25		1.004793

				314.27		1.004793

				314.29		1.004793

				314.31		1.004793

				314.34		1.004793

				314.36		1.004793

				314.38		1.004793

				314.4		1.004793

				314.42		1.004793

				314.44		1.004793

				314.46		1.000913

				314.48		1.000913

				314.51		1.000913

				314.53		1.000913

				314.55		1.000913

				314.57		1.000913

				314.59		1.000913

				314.61		1.000913

				314.63		1.000913

				314.65		1.000913

				314.67		1.000913

				314.7		1.000913

				314.72		1.000913

				314.74		1.000913

				314.76		1.000913

				314.78		1.000913

				314.8		1.000913

				314.82		1.000913

				314.84		1.000913

				314.86		1.000913

				314.89		0.9970327

				314.91		1.000913

				314.93		1.000913

				314.95		1.000913

				314.97		0.9970327

				314.99		1.000913

				315.01		1.000913

				315.03		0.9970327

				315.05		0.9970327

				315.08		0.9970327

				315.1		0.9970327

				315.12		0.9970327

				315.14		0.9970327

				315.16		0.9970327

				315.18		0.9970327

				315.2		0.9970327

				315.22		0.9970327

				315.24		0.9970327

				315.27		0.9970327

				315.29		0.9970327

				315.31		0.9970327

				315.33		0.9970327

				315.35		0.9970327

				315.37		0.9970327

				315.39		0.9970327

				315.41		0.9970327

				315.43		0.9931527

				315.46		0.9970327

				315.48		0.9931527

				315.5		0.9931527

				315.52		0.9931527

				315.54		0.9931527

				315.56		0.9931527

				315.58		0.9931527

				315.6		0.9931527

				315.62		0.9931527

				315.65		0.9931527

				315.67		0.9931527

				315.69		0.9931527

				315.71		0.9931527

				315.73		0.9931527

				315.75		0.9931527

				315.77		0.9931527

				315.79		0.9931527

				315.82		0.9931527

				315.84		0.9931527

				315.86		0.9931527

				315.88		0.9931527

				315.9		0.9931527

				315.92		0.9931527

				315.94		0.9931527

				315.96		0.9931527

				315.98		0.9931527

				316.01		0.9931527

				316.03		0.9931527

				316.05		0.9931527

				316.07		0.9931527

				316.09		0.9931527

				316.11		0.9931527

				316.13		0.9931527

				316.15		0.9931527

				316.17		0.9931527

				316.2		0.9931527

				316.22		0.9931527

				316.24		0.9931527

				316.26		0.9931527

				316.28		0.9931527

				316.3		0.9931527

				316.32		0.9892727

				316.34		0.9892727

				316.36		0.9892727

				316.39		0.9931527

				316.41		0.9892727

				316.43		0.9892727

				316.45		0.9892727

				316.47		0.9892727

				316.49		0.9931527

				316.51		0.9892727

				316.53		0.9892727

				316.55		0.9931527

				316.58		0.9931527

				316.6		0.9892727

				316.62		0.9892727

				316.64		0.9892727

				316.66		0.9892727

				316.68		0.9892727

				316.7		0.9892727

				316.72		0.9892727

				316.75		0.9892727

				316.77		0.9892727

				316.79		0.9892727

				316.81		0.9892727

				316.83		0.9892727

				316.85		0.9892727

				316.87		0.9892727

				316.89		0.9853926

				316.91		0.9892727

				316.94		0.9892727

				316.96		0.9853926

				316.98		0.9892727

				317		0.9853926

				317.02		0.9853926

				317.04		0.9853926

				317.06		0.9853926

				317.08		0.9853926

				317.1		0.9853926

				317.13		0.9853926

				317.15		0.9853926

				317.17		0.9853926

				317.19		0.9853926

				317.21		0.9853926

				317.23		0.9853926

				317.25		0.9853926

				317.27		0.9853926

				317.29		0.9853926

				317.32		0.9815126

				317.34		0.9853926

				317.36		0.9853926

				317.38		0.9853926

				317.4		0.9853926

				317.42		0.9853926

				317.44		0.9853926

				317.46		0.9853926

				317.49		0.9853926

				317.51		0.9853926

				317.53		0.9853926

				317.55		0.9853926

				317.57		0.9853926

				317.59		0.9853926

				317.61		0.9815126

				317.63		0.9853926

				317.65		0.9853926

				317.68		0.9853926

				317.7		0.9853926

				317.72		0.9853926

				317.74		0.9853926

				317.76		0.9815126

				317.78		0.9853926

				317.8		0.9815126

				317.82		0.9815126

				317.84		0.9815126

				317.87		0.9815126

				317.89		0.9815126

				317.91		0.9853926

				317.93		0.9853926

				317.95		0.9815126

				317.97		0.9815126

				317.99		0.9815126

				318.01		0.9815126

				318.04		0.9815126

				318.06		0.9815126

				318.08		0.9815126

				318.1		0.9815126

				318.12		0.9815126

				318.14		0.9815126

				318.16		0.9815126

				318.18		0.9815126

				318.2		0.9815126

				318.23		0.9815126

				318.25		0.9815126

				318.27		0.9815126

				318.29		0.9815126

				318.31		0.9815126

				318.33		0.9815126

				318.35		0.9815126

				318.37		0.9815126

				318.39		0.9853926

				318.42		0.9815126

				318.44		0.9853926

				318.46		0.9853926

				318.48		0.9853926

				318.5		0.9853926

				318.52		0.9815126

				318.54		0.9853926

				318.56		0.9853926

				318.59		0.9853926

				318.61		0.9853926

				318.63		0.9853926

				318.65		0.9853926

				318.67		0.9853926

				318.69		0.9853926

				318.71		0.9853926

				318.73		0.9853926

				318.75		0.9853926

				318.78		0.9853926

				318.8		0.9853926

				318.82		0.9853926

				318.84		0.9853926

				318.86		0.9853926

				318.88		0.9853926

				318.9		0.9892727

				318.92		0.9853926

				318.94		0.9853926

				318.97		0.9853926

				318.99		0.9892727

				319.01		0.9892727

				319.03		0.9892727

				319.05		0.9892727

				319.07		0.9892727

				319.09		0.9892727

				319.11		0.9892727

				319.14		0.9892727

				319.16		0.9892727

				319.18		0.9892727

				319.2		0.9892727

				319.22		0.9892727

				319.24		0.9892727

				319.26		0.9892727

				319.28		0.9892727

				319.3		0.9892727

				319.33		0.9892727

				319.35		0.9892727

				319.37		0.9892727

				319.39		0.9892727

				319.41		0.9892727

				319.43		0.9892727

				319.45		0.9892727

				319.47		0.9892727

				319.49		0.9892727

				319.52		0.9892727

				319.54		0.9892727

				319.56		0.9892727

				319.58		0.9892727

				319.6		0.9892727

				319.62		0.9892727

				319.64		0.9892727

				319.66		0.9892727

				319.68		0.9892727

				319.71		0.9892727

				319.73		0.9892727

				319.75		0.9892727

				319.77		0.9892727

				319.79		0.9892727

				319.81		0.9892727

				319.83		0.9892727

				319.85		0.9892727

				319.88		0.9892727

				319.9		0.9892727

				319.92		0.9892727

				319.94		0.9892727

				319.96		0.9892727

				319.98		0.9892727

				320		0.9892727

				320.02		0.9892727

				320.04		0.9892727

				320.07		0.9892727

				320.09		0.9892727

				320.11		0.9892727

				320.13		0.9892727

				320.15		0.9892727

				320.17		0.9892727

				320.19		0.9892727

				320.21		0.9892727

				320.23		0.9892727

				320.26		0.9892727

				320.28		0.9892727

				320.3		0.9892727

				320.32		0.9892727

				320.34		0.9892727

				320.36		0.9892727

				320.38		0.9892727

				320.4		0.9892727

				320.42		0.9892727

				320.45		0.9892727

				320.47		0.9892727

				320.49		0.9892727

				320.51		0.9892727

				320.53		0.9892727

				320.55		0.9892727

				320.57		0.9892727

				320.59		0.9892727

				320.61		0.9892727

				320.64		0.9892727

				320.66		0.9892727

				320.68		0.9892727

				320.7		0.9853926

				320.72		0.9892727

				320.74		0.9853926

				320.76		0.9853926

				320.78		0.9853926

				320.81		0.9853926

				320.83		0.9853926

				320.85		0.9853926

				320.87		0.9853926

				320.89		0.9853926

				320.91		0.9853926

				320.93		0.9853926

				320.95		0.9853926

				320.97		0.9853926

				321		0.9853926

				321.02		0.9853926

				321.04		0.9853926

				321.06		0.9853926

				321.08		0.9853926

				321.1		0.9853926

				321.12		0.9853926

				321.14		0.9853926

				321.16		0.9853926

				321.19		0.9853926

				321.21		0.9815126

				321.23		0.9815126

				321.25		0.9815126

				321.27		0.9815126

				321.29		0.9815126

				321.31		0.9815126

				321.33		0.9815126

				321.36		0.9815126

				321.38		0.9815126

				321.4		0.9815126

				321.42		0.9815126

				321.44		0.9815126

				321.46		0.9815126

				321.48		0.9815126

				321.5		0.9815126

				321.52		0.9815126

				321.55		0.9815126

				321.57		0.9815126

				321.59		0.9815126

				321.61		0.9815126

				321.63		0.9815126

				321.65		0.9815126

				321.67		0.9815126

				321.69		0.9815126

				321.72		0.9815126

				321.74		0.9815126

				321.76		0.9815126

				321.78		0.9815126

				321.8		0.9815126

				321.82		0.9815126

				321.84		0.9815126

				321.86		0.9815126

				321.88		0.9776326

				321.91		0.9776326

				321.93		0.9776326

				321.95		0.9776326

				321.97		0.9776326

				321.99		0.9776326

				322.01		0.9776326

				322.03		0.9776326

				322.05		0.9776326

				322.08		0.9776326

				322.1		0.9776326

				322.12		0.9776326

				322.14		0.9776326

				322.16		0.9776326

				322.18		0.9776326

				322.2		0.9776326

				322.22		0.9737525

				322.24		0.9737525

				322.27		0.9737525

				322.29		0.9737525

				322.31		0.9737525

				322.33		0.9737525

				322.35		0.9737525

				322.37		0.9737525

				322.39		0.9737525

				322.41		0.9737525

				322.44		0.9737525

				322.46		0.9737525

				322.48		0.9737525

				322.5		0.9737525

				322.52		0.9737525

				322.54		0.9737525

				322.56		0.9737525

				322.58		0.9737525

				322.6		0.9737525

				322.63		0.9737525

				322.65		0.9737525

				322.67		0.9737525

				322.69		0.9737525

				322.71		0.9737525

				322.73		0.9737525

				322.75		0.9737525

				322.77		0.9737525

				322.8		0.9737525

				322.82		0.9698725

				322.84		0.9737525

				322.86		0.9737525

				322.88		0.9737525

				322.9		0.9737525

				322.92		0.9737525

				322.94		0.9737525

				322.96		0.9737525

				322.99		0.9737525

				323.01		0.9698725

				323.03		0.9737525

				323.05		0.9698725

				323.07		0.9698725

				323.09		0.9698725

				323.11		0.9698725

				323.13		0.9698725

				323.15		0.9698725

				323.18		0.9698725

				323.2		0.9698725

				323.22		0.9698725

				323.24		0.9698725

				323.26		0.9659924

				323.28		0.9659924

				323.3		0.9659924

				323.32		0.9698725

				323.35		0.9698725

				323.37		0.9698725

				323.39		0.9698725

				323.41		0.9698725

				323.43		0.9698725

				323.45		0.9698725

				323.47		0.9698725

				323.49		0.9659924

				323.51		0.9659924

				323.54		0.9659924

				323.56		0.9659924

				323.58		0.9659924

				323.6		0.9659924

				323.62		0.9659924

				323.64		0.9659924

				323.66		0.9659924

				323.68		0.9659924

				323.71		0.9659924

				323.73		0.9659924

				323.75		0.9659924

				323.77		0.9659924

				323.79		0.9659924

				323.81		0.9659924

				323.83		0.9659924

				323.85		0.9659924

				323.87		0.9659924

				323.9		0.9659924

				323.92		0.9659924

				323.94		0.9659924

				323.96		0.9659924

				323.98		0.9659924

				324		0.9659924

				324.02		0.9659924

				324.04		0.9659924

				324.07		0.9659924

				324.09		0.9659924

				324.11		0.9659924

				324.13		0.9659924

				324.15		0.9659924

				324.17		0.9659924

				324.19		0.9659924

				324.21		0.9659924

				324.23		0.9659924

				324.26		0.9659924

				324.28		0.9659924

				324.3		0.9659924

				324.32		0.9659924

				324.34		0.9659924

				324.36		0.9659924

				324.38		0.9659924

				324.4		0.9659924

				324.43		0.9659924

				324.45		0.9659924

				324.47		0.9659924

				324.49		0.9659924

				324.51		0.9659924

				324.53		0.9659924

				324.55		0.9659924

				324.57		0.9659924

				324.59		0.9659924

				324.62		0.9659924

				324.64		0.9659924

				324.66		0.9659924

				324.68		0.9659924

				324.7		0.9659924

				324.72		0.9659924

				324.74		0.9659924

				324.76		0.9659924

				324.79		0.9659924

				324.81		0.9659924

				324.83		0.9659924

				324.85		0.9659924

				324.87		0.9659924

				324.89		0.9659924

				324.91		0.9659924

				324.93		0.9659924

				324.95		0.9659924

				324.98		0.9659924

				325		0.9659924

				325.02		0.9659924

				325.04		0.9621124

				325.06		0.9621124

				325.08		0.9621124

				325.1		0.9621124

				325.12		0.9621124

				325.15		0.9621124

				325.17		0.9621124

				325.19		0.9621124

				325.21		0.9621124

				325.23		0.9621124

				325.25		0.9621124

				325.27		0.9659924

				325.29		0.9659924

				325.32		0.9621124

				325.34		0.9659924

				325.36		0.9659924

				325.38		0.9659924

				325.4		0.9659924

				325.42		0.9659924

				325.44		0.9659924

				325.46		0.9659924

				325.48		0.9659924

				325.51		0.9659924

				325.53		0.9659924

				325.55		0.9659924

				325.57		0.9659924

				325.59		0.9659924

				325.61		0.9659924

				325.63		0.9659924

				325.65		0.9659924

				325.68		0.9659924

				325.7		0.9659924

				325.72		0.9659924

				325.74		0.9659924

				325.76		0.9659924

				325.78		0.9659924

				325.8		0.9659924

				325.82		0.9621124

				325.84		0.9621124

				325.87		0.9621124

				325.89		0.9621124

				325.91		0.9621124

				325.93		0.9621124

				325.95		0.9621124

				325.97		0.9621124

				325.99		0.9621124

				326.01		0.9621124

				326.04		0.9621124

				326.06		0.9621124

				326.08		0.9621124

				326.1		0.9582324

				326.12		0.9621124

				326.14		0.9582324

				326.16		0.9582324

				326.18		0.9582324

				326.21		0.9582324

				326.23		0.9582324

				326.25		0.9582324

				326.27		0.9582324

				326.29		0.9582324

				326.31		0.9582324

				326.33		0.9582324

				326.35		0.9582324

				326.38		0.9582324

				326.4		0.9582324

				326.42		0.9582324

				326.44		0.9582324

				326.46		0.9582324

				326.48		0.9582324

				326.5		0.9582324

				326.52		0.9582324

				326.54		0.9582324

				326.57		0.9582324

				326.59		0.9582324

				326.61		0.9582324

				326.63		0.9582324

				326.65		0.9582324

				326.67		0.9582324

				326.69		0.9582324

				326.71		0.9582324

				326.74		0.9582324

				326.76		0.9582324

				326.78		0.9582324

				326.8		0.9582324

				326.82		0.9582324

				326.84		0.9582324

				326.86		0.9582324

				326.88		0.9582324

				326.91		0.9582324

				326.93		0.9582324

				326.95		0.9582324

				326.97		0.9543523

				326.99		0.9543523

				327.01		0.9543523

				327.03		0.9543523

				327.05		0.9543523

				327.08		0.9582324

				327.1		0.9582324

				327.12		0.9582324

				327.14		0.9582324

				327.16		0.9582324

				327.18		0.9582324

				327.2		0.9582324

				327.22		0.9582324

				327.25		0.9582324

				327.27		0.9582324

				327.29		0.9582324

				327.31		0.9582324

				327.33		0.9582324

				327.35		0.9582324

				327.37		0.9582324

				327.39		0.9582324

				327.41		0.9582324

				327.44		0.9582324

				327.46		0.9582324

				327.48		0.9582324

				327.5		0.9582324

				327.52		0.9582324

				327.54		0.9543523

				327.56		0.9582324

				327.58		0.9543523

				327.61		0.9543523

				327.63		0.9543523

				327.65		0.9543523

				327.67		0.9543523

				327.69		0.9543523

				327.71		0.9543523

				327.73		0.9543523

				327.75		0.9543523

				327.78		0.9543523

				327.8		0.9543523

				327.82		0.9543523

				327.84		0.9543523

				327.86		0.9543523

				327.88		0.9543523

				327.9		0.9543523

				327.92		0.9543523

				327.95		0.9543523

				327.97		0.9582324

				327.99		0.9543523

				328.01		0.9582324

				328.03		0.9582324

				328.05		0.9543523

				328.07		0.9582324

				328.09		0.9582324

				328.12		0.9582324

				328.14		0.9582324

				328.16		0.9582324

				328.18		0.9582324

				328.2		0.9582324

				328.22		0.9582324

				328.24		0.9582324

				328.26		0.9582324

				328.28		0.9582324

				328.31		0.9582324

				328.33		0.9582324

				328.35		0.9582324

				328.37		0.9582324

				328.39		0.9582324

				328.41		0.9582324

				328.43		0.9582324

				328.45		0.9582324

				328.48		0.9582324

				328.5		0.9582324

				328.52		0.9582324

				328.54		0.9582324

				328.56		0.9582324

				328.58		0.9582324

				328.6		0.9582324

				328.62		0.9582324

				328.65		0.9582324

				328.67		0.9582324

				328.69		0.9582324

				328.71		0.9582324

				328.73		0.9582324

				328.75		0.9582324

				328.77		0.9582324

				328.79		0.9582324

				328.81		0.9582324

				328.84		0.9582324

				328.86		0.9582324

				328.88		0.9582324

				328.9		0.9582324

				328.92		0.9582324

				328.94		0.9582324

				328.96		0.9582324

				328.98		0.9582324

				329.01		0.9582324

				329.03		0.9582324

				329.05		0.9582324

				329.07		0.9582324

				329.09		0.9582324

				329.11		0.9582324

				329.13		0.9582324

				329.15		0.9582324

				329.18		0.9582324

				329.2		0.9582324

				329.22		0.9582324

				329.24		0.9582324

				329.26		0.9582324

				329.28		0.9582324

				329.3		0.9582324

				329.32		0.9582324

				329.34		0.9582324

				329.37		0.9582324

				329.39		0.9582324

				329.41		0.9582324

				329.43		0.9543523

				329.45		0.9582324

				329.47		0.9543523

				329.49		0.9543523

				329.51		0.9543523

				329.54		0.9543523

				329.56		0.9543523

				329.58		0.9543523

				329.6		0.9543523

				329.62		0.9543523

				329.64		0.9543523

				329.66		0.9543523

				329.68		0.9582324

				329.7		0.9582324

				329.73		0.9582324

				329.75		0.9582324

				329.77		0.9582324

				329.79		0.9543523

				329.81		0.9543523

				329.83		0.9543523

				329.85		0.9582324

				329.87		0.9543523

				329.9		0.9582324

				329.92		0.9582324

				329.94		0.9543523

				329.96		0.9582324

				329.98		0.9582324

				330		0.9543523

				330.02		0.9543523

				330.04		0.9582324

				330.06		0.9543523

				330.09		0.9543523

				330.11		0.9543523

				330.13		0.9543523

				330.15		0.9543523

				330.17		0.9543523

				330.19		0.9543523

				330.21		0.9543523

				330.23		0.9543523

				330.26		0.9543523

				330.28		0.9543523

				330.3		0.9543523

				330.32		0.9543523

				330.34		0.9543523

				330.36		0.9543523

				330.38		0.9543523

				330.4		0.9543523

				330.43		0.9543523

				330.45		0.9543523

				330.47		0.9543523

				330.49		0.9543523

				330.51		0.9543523

				330.53		0.9543523

				330.55		0.9543523

				330.57		0.9543523

				330.59		0.9543523

				330.62		0.9543523

				330.64		0.9543523

				330.66		0.9543523

				330.68		0.9543523

				330.7		0.9543523

				330.72		0.9543523

				330.74		0.9543523

				330.76		0.9543523

				330.79		0.9543523

				330.81		0.9543523

				330.83		0.9543523

				330.85		0.9543523

				330.87		0.9543523

				330.89		0.9543523

				330.91		0.9543523

				330.93		0.9543523

				330.95		0.9504723

				330.98		0.9543523

				331		0.9504723

				331.02		0.9504723

				331.04		0.9504723

				331.06		0.9504723

				331.08		0.9504723

				331.1		0.9543523

				331.12		0.9543523

				331.15		0.9543523

				331.17		0.9543523

				331.19		0.9543523

				331.21		0.9543523

				331.23		0.9543523

				331.25		0.9543523

				331.27		0.9543523

				331.29		0.9543523

				331.31		0.9543523

				331.34		0.9543523

				331.36		0.9543523

				331.38		0.9543523

				331.4		0.9543523

				331.42		0.9543523

				331.44		0.9543523

				331.46		0.9543523

				331.48		0.9543523

				331.5		0.9543523

				331.53		0.9543523

				331.55		0.9543523

				331.57		0.9543523

				331.59		0.9543523

				331.61		0.9543523

				331.63		0.9543523

				331.65		0.9543523

				331.67		0.9543523

				331.7		0.9543523

				331.72		0.9543523

				331.74		0.9543523

				331.76		0.9543523

				331.78		0.9543523

				331.8		0.9543523

				331.82		0.9543523

				331.84		0.9504723

				331.87		0.9543523

				331.89		0.9543523

				331.91		0.9543523

				331.93		0.9543523

				331.95		0.9543523

				331.97		0.9504723

				331.99		0.9504723

				332.01		0.9504723

				332.03		0.9543523

				332.06		0.9504723

				332.08		0.9543523

				332.1		0.9504723

				332.12		0.9504723

				332.14		0.9504723

				332.16		0.9504723

				332.18		0.9504723

				332.2		0.9504723

				332.23		0.9504723

				332.25		0.9504723

				332.27		0.9504723

				332.29		0.9504723

				332.31		0.9504723

				332.33		0.9504723

				332.35		0.9504723

				332.37		0.9504723

				332.4		0.9504723

				332.42		0.9504723

				332.44		0.9504723

				332.46		0.9504723

				332.48		0.9504723

				332.5		0.9504723

				332.52		0.9504723

				332.54		0.9504723

				332.56		0.9504723

				332.59		0.9504723

				332.61		0.9504723

				332.63		0.9504723

				332.65		0.9504723

				332.67		0.9504723

				332.69		0.9504723

				332.71		0.9504723

				332.73		0.9504723

				332.76		0.9504723

				332.78		0.9504723

				332.8		0.9465923

				332.82		0.9465923

				332.84		0.9465923

				332.86		0.9465923

				332.88		0.9465923

				332.9		0.9465923

				332.93		0.9465923

				332.95		0.9465923

				332.97		0.9465923

				332.99		0.9504723

				333.01		0.9504723

				333.03		0.9504723

				333.05		0.9504723

				333.07		0.9504723

				333.09		0.9504723

				333.12		0.9504723

				333.14		0.9504723

				333.16		0.9504723

				333.18		0.9504723

				333.2		0.9504723

				333.22		0.9504723

				333.24		0.9465923

				333.26		0.9504723

				333.29		0.9465923

				333.31		0.9504723

				333.33		0.9465923

				333.35		0.9504723

				333.37		0.9504723

				333.39		0.9465923

				333.41		0.9504723

				333.43		0.9504723

				333.46		0.9504723

				333.48		0.9504723

				333.5		0.9504723

				333.52		0.9504723

				333.54		0.9504723

				333.56		0.9504723

				333.58		0.9504723

				333.6		0.9504723

				333.63		0.9504723

				333.65		0.9504723

				333.67		0.9504723

				333.69		0.9504723

				333.71		0.9504723

				333.73		0.9504723

				333.75		0.9504723

				333.77		0.9504723

				333.79		0.9504723

				333.82		0.9504723

				333.84		0.9504723

				333.86		0.9504723

				333.88		0.9504723

				333.9		0.9504723

				333.92		0.9504723

				333.94		0.9543523

				333.96		0.9504723

				333.99		0.9543523

				334.01		0.9504723

				334.03		0.9504723

				334.05		0.9504723

				334.07		0.9543523

				334.09		0.9543523

				334.11		0.9543523

				334.13		0.9543523

				334.16		0.9543523

				334.18		0.9504723

				334.2		0.9543523

				334.22		0.9543523

				334.24		0.9543523

				334.26		0.9543523

				334.28		0.9504723

				334.3		0.9543523

				334.32		0.9543523

				334.35		0.9543523

				334.37		0.9543523

				334.39		0.9543523

				334.41		0.9543523

				334.43		0.9543523

				334.45		0.9543523

				334.47		0.9543523

				334.49		0.9543523

				334.52		0.9543523

				334.54		0.9543523

				334.56		0.9543523

				334.58		0.9543523

				334.6		0.9543523

				334.62		0.9543523

				334.64		0.9543523

				334.66		0.9543523

				334.68		0.9543523

				334.71		0.9543523

				334.73		0.9543523

				334.75		0.9543523

				334.77		0.9543523

				334.79		0.9543523

				334.81		0.9543523

				334.83		0.9543523

				334.85		0.9543523

				334.88		0.9543523

				334.9		0.9543523

				334.92		0.9543523

				334.94		0.9543523

				334.96		0.9543523

				334.98		0.9543523

				335		0.9582324

				335.02		0.9582324

				335.04		0.9543523

				335.07		0.9582324

				335.09		0.9543523

				335.11		0.9543523

				335.13		0.9543523

				335.15		0.9543523

				335.17		0.9543523

				335.19		0.9543523

				335.21		0.9543523

				335.24		0.9543523

				335.26		0.9543523

				335.28		0.9543523

				335.3		0.9543523

				335.32		0.9543523

				335.34		0.9543523

				335.36		0.9543523

				335.38		0.9543523

				335.41		0.9543523

				335.43		0.9543523

				335.45		0.9543523

				335.47		0.9543523

				335.49		0.9543523

				335.51		0.9543523

				335.53		0.9543523

				335.55		0.9543523

				335.57		0.9543523

				335.6		0.9543523

				335.62		0.9504723

				335.64		0.9504723

				335.66		0.9504723

				335.68		0.9504723

				335.7		0.9504723

				335.72		0.9504723

				335.74		0.9504723

				335.76		0.9504723

				335.79		0.9504723

				335.81		0.9504723

				335.83		0.9504723

				335.85		0.9504723

				335.87		0.9504723

				335.89		0.9504723

				335.91		0.9504723

				335.93		0.9504723

				335.96		0.9504723

				335.98		0.9504723

				336		0.9465923

				336.02		0.9465923

				336.04		0.9465923

				336.06		0.9465923

				336.08		0.9465923

				336.1		0.9504723

				336.12		0.9504723

				336.15		0.9504723

				336.17		0.9465923

				336.19		0.9465923

				336.21		0.9504723

				336.23		0.9504723

				336.25		0.9465923

				336.27		0.9504723

				336.29		0.9465923

				336.32		0.9465923

				336.34		0.9465923

				336.36		0.9465923

				336.38		0.9465923

				336.4		0.9465923

				336.42		0.9465923

				336.44		0.9465923

				336.46		0.9465923

				336.48		0.9465923

				336.51		0.9465923

				336.53		0.9465923

				336.55		0.9465923

				336.57		0.9465923

				336.59		0.9465923

				336.61		0.9465923

				336.63		0.9465923

				336.65		0.9465923

				336.67		0.9465923

				336.7		0.9465923

				336.72		0.9427122

				336.74		0.9465923

				336.76		0.9427122

				336.78		0.9427122

				336.8		0.9465923

				336.82		0.9427122

				336.84		0.9427122

				336.87		0.9427122

				336.89		0.9427122

				336.91		0.9427122

				336.93		0.9427122

				336.95		0.9427122

				336.97		0.9427122

				336.99		0.9427122

				337.01		0.9427122

				337.03		0.9427122

				337.06		0.9427122

				337.08		0.9427122

				337.1		0.9427122

				337.12		0.9427122

				337.14		0.9427122

				337.16		0.9427122

				337.18		0.9427122

				337.2		0.9427122

				337.23		0.9388322

				337.25		0.9388322

				337.27		0.9388322

				337.29		0.9388322

				337.31		0.9388322

				337.33		0.9388322

				337.35		0.9388322

				337.37		0.9388322

				337.39		0.9388322

				337.42		0.9388322

				337.44		0.9388322

				337.46		0.9388322

				337.48		0.9388322

				337.5		0.9388322

				337.52		0.9388322

				337.54		0.9388322

				337.56		0.9388322

				337.59		0.9388322

				337.61		0.9388322

				337.63		0.9388322

				337.65		0.9388322

				337.67		0.9388322

				337.69		0.9388322

				337.71		0.9388322

				337.73		0.9388322

				337.75		0.9388322

				337.78		0.9388322

				337.8		0.9388322

				337.82		0.9388322

				337.84		0.9388322

				337.86		0.9388322

				337.88		0.9388322

				337.9		0.9388322

				337.92		0.9388322

				337.94		0.9388322

				337.97		0.9388322

				337.99		0.9388322

				338.01		0.9388322

				338.03		0.9388322

				338.05		0.9388322

				338.07		0.9388322

				338.09		0.9388322

				338.11		0.9388322

				338.14		0.9388322

				338.16		0.9388322

				338.18		0.9388322

				338.2		0.9388322

				338.22		0.9349522

				338.24		0.9349522

				338.26		0.9388322

				338.28		0.9349522

				338.31		0.9349522

				338.33		0.9349522

				338.35		0.9349522

				338.37		0.9349522

				338.39		0.9349522

				338.41		0.9349522

				338.43		0.9349522

				338.45		0.9349522

				338.47		0.9349522

				338.5		0.9349522

				338.52		0.9349522

				338.54		0.9349522

				338.56		0.9349522

				338.58		0.9349522

				338.6		0.9349522

				338.62		0.9349522

				338.64		0.9349522

				338.66		0.9349522

				338.69		0.9349522

				338.71		0.9349522

				338.73		0.9349522

				338.75		0.9349522

				338.77		0.9349522

				338.79		0.9349522

				338.81		0.9349522

				338.83		0.9349522

				338.86		0.9349522

				338.88		0.9349522

				338.9		0.9349522

				338.92		0.9349522

				338.94		0.9349522

				338.96		0.9349522

				338.98		0.9349522

				339		0.9349522

				339.02		0.9349522

				339.05		0.9349522

				339.07		0.9349522

				339.09		0.9349522

				339.11		0.9349522

				339.13		0.9349522

				339.15		0.9349522

				339.17		0.9349522

				339.19		0.9349522

				339.22		0.9349522

				339.24		0.9310721

				339.26		0.9310721

				339.28		0.9310721

				339.3		0.9310721

				339.32		0.9310721

				339.34		0.9310721

				339.36		0.9310721

				339.38		0.9310721

				339.41		0.9310721

				339.43		0.9310721

				339.45		0.9310721

				339.47		0.9310721

				339.49		0.9310721

				339.51		0.9310721

				339.53		0.9310721

				339.55		0.9310721

				339.57		0.9310721

				339.6		0.9310721

				339.62		0.9310721

				339.64		0.9310721

				339.66		0.9310721

				339.68		0.9310721

				339.7		0.9310721

				339.72		0.9310721

				339.74		0.9310721

				339.76		0.9310721

				339.79		0.9310721

				339.81		0.9310721

				339.83		0.9310721

				339.85		0.9310721

				339.87		0.9310721

				339.89		0.9310721

				339.91		0.9310721

				339.93		0.9310721

				339.96		0.9349522

				339.98		0.9310721

				340		0.9310721

				340.02		0.9310721

				340.04		0.9349522

				340.06		0.9349522

				340.08		0.9349522

				340.1		0.9310721

				340.12		0.9310721

				340.15		0.9310721

				340.17		0.9349522

				340.19		0.9310721

				340.21		0.9310721

				340.23		0.9310721

				340.25		0.9310721

				340.27		0.9310721

				340.29		0.9310721

				340.31		0.9349522

				340.34		0.9349522

				340.36		0.9349522

				340.38		0.9349522

				340.4		0.9349522

				340.42		0.9349522

				340.44		0.9349522

				340.46		0.9349522

				340.48		0.9349522

				340.5		0.9349522

				340.53		0.9349522

				340.55		0.9349522

				340.57		0.9349522

				340.59		0.9349522

				340.61		0.9349522

				340.63		0.9349522

				340.65		0.9349522

				340.67		0.9349522

				340.69		0.9349522

				340.72		0.9349522

				340.74		0.9349522

				340.76		0.9310721

				340.78		0.9349522

				340.8		0.9349522

				340.82		0.9349522

				340.84		0.9310721

				340.86		0.9349522

				340.89		0.9310721

				340.91		0.9310721

				340.93		0.9349522

				340.95		0.9310721

				340.97		0.9310721

				340.99		0.9310721

				341.01		0.9310721

				341.03		0.9310721

				341.05		0.9310721

				341.08		0.9310721

				341.1		0.9310721

				341.12		0.9310721

				341.14		0.9310721

				341.16		0.9310721

				341.18		0.9310721

				341.2		0.9310721

				341.22		0.9310721

				341.24		0.9310721

				341.27		0.9310721

				341.29		0.9310721

				341.31		0.9310721

				341.33		0.9310721

				341.35		0.9310721

				341.37		0.9310721

				341.39		0.9310721

				341.41		0.9310721

				341.43		0.9310721

				341.46		0.9310721

				341.48		0.9310721

				341.5		0.9310721

				341.52		0.9310721

				341.54		0.9310721

				341.56		0.9310721

				341.58		0.9310721

				341.6		0.9310721

				341.62		0.9310721

				341.65		0.9310721

				341.67		0.9310721

				341.69		0.9310721

				341.71		0.9310721

				341.73		0.9310721

				341.75		0.9310721

				341.77		0.9310721

				341.79		0.9310721

				341.81		0.9271921

				341.84		0.9271921

				341.86		0.9271921

				341.88		0.9271921

				341.9		0.9271921

				341.92		0.9271921

				341.94		0.9271921

				341.96		0.9271921

				341.98		0.9271921

				342		0.9271921

				342.03		0.9271921

				342.05		0.9271921

				342.07		0.9271921

				342.09		0.9271921

				342.11		0.9271921

				342.13		0.9271921

				342.15		0.9233121

				342.17		0.9233121

				342.19		0.9233121

				342.22		0.9233121

				342.24		0.9233121

				342.26		0.9233121

				342.28		0.9233121

				342.3		0.9233121

				342.32		0.9233121

				342.34		0.9233121

				342.36		0.9233121

				342.38		0.9233121

				342.41		0.9233121

				342.43		0.9233121

				342.45		0.9233121

				342.47		0.9233121

				342.49		0.9233121

				342.51		0.9233121

				342.53		0.9233121

				342.55		0.9233121

				342.57		0.9233121

				342.6		0.9233121

				342.62		0.9233121

				342.64		0.9233121

				342.66		0.9233121

				342.68		0.9233121

				342.7		0.9233121

				342.72		0.9233121

				342.74		0.9233121

				342.76		0.919432

				342.79		0.919432

				342.81		0.919432

				342.83		0.919432

				342.85		0.919432

				342.87		0.919432

				342.89		0.919432

				342.91		0.919432

				342.93		0.919432

				342.95		0.919432

				342.98		0.919432

				343		0.919432

				343.02		0.919432

				343.04		0.919432

				343.06		0.919432

				343.08		0.915552

				343.1		0.919432

				343.12		0.915552

				343.14		0.915552

				343.17		0.919432

				343.19		0.915552

				343.21		0.915552

				343.23		0.915552

				343.25		0.915552

				343.27		0.915552

				343.29		0.915552

				343.31		0.915552

				343.33		0.915552

				343.36		0.915552

				343.38		0.915552

				343.4		0.915552

				343.42		0.915552

				343.44		0.915552

				343.46		0.915552

				343.48		0.915552

				343.5		0.915552

				343.52		0.915552

				343.55		0.915552

				343.57		0.915552

				343.59		0.915552

				343.61		0.915552

				343.63		0.915552

				343.65		0.915552

				343.67		0.915552

				343.69		0.915552

				343.71		0.915552

				343.74		0.919432

				343.76		0.919432

				343.78		0.915552

				343.8		0.919432

				343.82		0.919432

				343.84		0.919432

				343.86		0.919432

				343.88		0.919432

				343.9		0.919432

				343.93		0.919432

				343.95		0.919432

				343.97		0.919432

				343.99		0.919432

				344.01		0.919432

				344.03		0.919432

				344.05		0.919432

				344.07		0.919432

				344.1		0.919432

				344.12		0.919432

				344.14		0.919432

				344.16		0.919432

				344.18		0.919432

				344.2		0.919432

				344.22		0.915552

				344.24		0.919432

				344.26		0.915552

				344.29		0.915552

				344.31		0.915552

				344.33		0.915552

				344.35		0.919432

				344.37		0.915552

				344.39		0.915552

				344.41		0.915552

				344.43		0.915552

				344.45		0.915552

				344.48		0.915552

				344.5		0.915552

				344.52		0.915552

				344.54		0.915552

				344.56		0.915552

				344.58		0.915552

				344.6		0.915552

				344.62		0.915552

				344.64		0.919432

				344.67		0.919432

				344.69		0.915552

				344.71		0.919432

				344.73		0.919432

				344.75		0.919432

				344.77		0.919432

				344.79		0.919432

				344.81		0.919432

				344.83		0.919432

				344.86		0.919432

				344.88		0.919432

				344.9		0.919432

				344.92		0.919432

				344.94		0.919432

				344.96		0.919432

				344.98		0.919432

				345		0.919432

				345.02		0.919432

				345.05		0.919432

				345.07		0.919432

				345.09		0.919432

				345.11		0.919432

				345.13		0.919432

				345.15		0.919432

				345.17		0.919432

				345.19		0.919432

				345.21		0.919432

				345.24		0.919432

				345.26		0.919432

				345.28		0.919432

				345.3		0.919432

				345.32		0.919432

				345.34		0.9233121

				345.36		0.919432

				345.38		0.919432

				345.41		0.919432

				345.43		0.919432

				345.45		0.919432

				345.47		0.919432

				345.49		0.919432

				345.51		0.919432

				345.53		0.919432

				345.55		0.919432

				345.57		0.919432

				345.6		0.919432

				345.62		0.919432

				345.64		0.919432

				345.66		0.919432

				345.68		0.919432

				345.7		0.919432

				345.72		0.919432

				345.74		0.919432

				345.76		0.919432

				345.79		0.919432

				345.81		0.919432

				345.83		0.919432

				345.85		0.919432

				345.87		0.919432

				345.89		0.919432

				345.91		0.919432

				345.93		0.919432

				345.95		0.919432

				345.98		0.919432

				346		0.919432

				346.02		0.919432

				346.04		0.919432

				346.06		0.919432

				346.08		0.919432

				346.1		0.919432

				346.12		0.919432

				346.14		0.919432

				346.17		0.919432

				346.19		0.919432

				346.21		0.919432

				346.23		0.919432

				346.25		0.919432

				346.27		0.919432

				346.29		0.919432

				346.31		0.919432

				346.33		0.919432

				346.36		0.919432

				346.38		0.9233121

				346.4		0.9233121

				346.42		0.9233121

				346.44		0.9233121

				346.46		0.9233121

				346.48		0.9233121

				346.5		0.9233121

				346.52		0.9233121

				346.55		0.9233121

				346.57		0.9233121

				346.59		0.9233121

				346.61		0.9233121

				346.63		0.9233121

				346.65		0.9233121

				346.67		0.9233121

				346.69		0.9233121

				346.71		0.9233121

				346.74		0.9233121

				346.76		0.9233121

				346.78		0.9233121

				346.8		0.9233121

				346.82		0.9233121

				346.84		0.9233121

				346.86		0.9233121

				346.88		0.919432

				346.9		0.919432

				346.93		0.9233121

				346.95		0.919432

				346.97		0.919432

				346.99		0.919432

				347.01		0.919432

				347.03		0.919432

				347.05		0.919432

				347.07		0.9233121

				347.09		0.9233121

				347.12		0.9233121

				347.14		0.919432

				347.16		0.919432

				347.18		0.919432

				347.2		0.9233121

				347.22		0.9233121

				347.24		0.9233121

				347.26		0.9233121

				347.28		0.919432

				347.31		0.9233121

				347.33		0.9233121

				347.35		0.9233121

				347.37		0.9233121

				347.39		0.9233121

				347.41		0.919432

				347.43		0.919432

				347.45		0.919432

				347.47		0.9233121

				347.5		0.919432

				347.52		0.9233121

				347.54		0.919432

				347.56		0.9233121

				347.58		0.9233121

				347.6		0.9233121

				347.62		0.9233121

				347.64		0.9233121

				347.66		0.9233121

				347.69		0.9233121

				347.71		0.9233121

				347.73		0.9233121

				347.75		0.9233121

				347.77		0.9233121

				347.79		0.9233121

				347.81		0.919432

				347.83		0.919432

				347.85		0.9233121

				347.88		0.919432

				347.9		0.919432

				347.92		0.919432

				347.94		0.919432

				347.96		0.919432

				347.98		0.919432

				348		0.919432

				348.02		0.919432

				348.04		0.919432

				348.07		0.919432

				348.09		0.919432

				348.11		0.919432

				348.13		0.919432

				348.15		0.919432

				348.17		0.919432

				348.19		0.919432

				348.21		0.919432

				348.23		0.919432

				348.26		0.919432

				348.28		0.919432

				348.3		0.919432

				348.32		0.919432

				348.34		0.919432

				348.36		0.919432

				348.38		0.915552

				348.4		0.919432

				348.42		0.915552

				348.44		0.915552

				348.47		0.915552

				348.49		0.915552

				348.51		0.915552

				348.53		0.915552

				348.55		0.915552

				348.57		0.915552

				348.59		0.915552

				348.61		0.915552

				348.64		0.915552

				348.66		0.915552

				348.68		0.915552

				348.7		0.915552

				348.72		0.911672

				348.74		0.911672

				348.76		0.911672

				348.78		0.911672

				348.8		0.911672

				348.83		0.911672

				348.85		0.911672

				348.87		0.911672

				348.89		0.911672

				348.91		0.9077919

				348.93		0.9077919

				348.95		0.9077919

				348.97		0.9077919

				348.99		0.9077919

				349.02		0.9077919

				349.04		0.9077919

				349.06		0.9077919

				349.08		0.9077919

				349.1		0.9077919

				349.12		0.9077919

				349.14		0.9077919

				349.16		0.9077919

				349.18		0.9077919

				349.21		0.9077919

				349.23		0.9077919

				349.25		0.9077919

				349.27		0.9077919

				349.29		0.9077919

				349.31		0.9077919

				349.33		0.9039119

				349.35		0.9039119

				349.38		0.9039119

				349.4		0.9039119

				349.42		0.9039119

				349.44		0.9039119

				349.46		0.9039119

				349.48		0.9039119

				349.5		0.9039119

				349.52		0.9039119

				349.55		0.9039119

				349.57		0.9039119

				349.59		0.9039119

				349.61		0.9039119

				349.63		0.9039119

				349.65		0.9039119

				349.67		0.9039119

				349.7		0.9039119

				349.72		0.9039119

				349.74		0.9039119

				349.76		0.9039119

				349.78		0.9000319

				349.8		0.9039119

				349.82		0.9000319

				349.84		0.9000319

				349.87		0.9000319

				349.89		0.9000319

				349.91		0.9000319

				349.93		0.9000319

				349.95		0.9000319

				349.97		0.9000319

				349.99		0.9000319

				350.02		0.9000319

				350.04		0.9000319

				350.06		0.9000319

				350.08		0.9000319

				350.1		0.9000319

				350.12		0.9000319

				350.14		0.9000319

				350.16		0.9000319

				350.19		0.9000319

				350.21		0.9000319

				350.23		0.9000319

				350.25		0.9000319

				350.27		0.9000319

				350.29		0.9000319

				350.31		0.9000319

				350.33		0.8961518

				350.36		0.8961518

				350.38		0.8961518

				350.4		0.8961518

				350.42		0.8961518

				350.44		0.8961518

				350.46		0.8961518

				350.48		0.8961518

				350.5		0.8961518

				350.53		0.8961518

				350.55		0.8961518

				350.57		0.8961518

				350.59		0.8961518

				350.61		0.8961518

				350.63		0.8961518

				350.65		0.8961518

				350.67		0.8961518

				350.69		0.8961518

				350.72		0.8961518

				350.74		0.8961518

				350.76		0.8961518

				350.78		0.8961518

				350.8		0.8961518

				350.82		0.8961518

				350.84		0.8961518

				350.86		0.8961518

				350.89		0.8961518

				350.91		0.8961518

				350.93		0.8961518

				350.95		0.8961518

				350.97		0.8961518

				350.99		0.8961518

				351.01		0.8961518

				351.03		0.9000319

				351.05		0.8961518

				351.08		0.8961518

				351.1		0.8961518

				351.12		0.8961518

				351.14		0.8961518

				351.16		0.8961518

				351.18		0.8961518

				351.2		0.8961518

				351.22		0.8961518

				351.24		0.8961518

				351.27		0.8961518

				351.29		0.8961518

				351.31		0.8961518

				351.33		0.8961518

				351.35		0.8961518

				351.37		0.8961518

				351.39		0.8922718

				351.41		0.8922718

				351.43		0.8922718

				351.46		0.8922718

				351.48		0.8922718

				351.5		0.8922718

				351.52		0.8922718

				351.54		0.8922718

				351.56		0.8922718

				351.58		0.8961518

				351.6		0.8961518

				351.63		0.8961518

				351.65		0.8922718

				351.67		0.8922718

				351.69		0.8922718

				351.71		0.8922718

				351.73		0.8922718

				351.75		0.8922718

				351.77		0.8922718

				351.79		0.8922718

				351.82		0.8922718

				351.84		0.8922718

				351.86		0.8922718

				351.88		0.8922718

				351.9		0.8883918

				351.92		0.8883918

				351.94		0.8883918

				351.96		0.8883918

				351.99		0.8883918

				352.01		0.8883918

				352.03		0.8883918

				352.05		0.8883918

				352.07		0.8883918

				352.09		0.8883918

				352.11		0.8883918

				352.13		0.8883918

				352.15		0.8883918

				352.18		0.8883918

				352.2		0.8883918

				352.22		0.8883918

				352.24		0.8883918

				352.26		0.8883918

				352.28		0.8883918

				352.3		0.8883918

				352.32		0.8845117

				352.35		0.8845117

				352.37		0.8845117

				352.39		0.8845117

				352.41		0.8845117

				352.43		0.8845117

				352.45		0.8845117

				352.47		0.8845117

				352.49		0.8845117

				352.52		0.8845117

				352.54		0.8845117

				352.56		0.8845117

				352.58		0.8845117

				352.6		0.8845117

				352.62		0.8845117

				352.64		0.8845117

				352.66		0.8845117

				352.69		0.8845117

				352.71		0.8845117

				352.73		0.8845117

				352.75		0.8845117

				352.77		0.8845117

				352.79		0.8806317

				352.81		0.8806317

				352.83		0.8806317

				352.85		0.8845117

				352.88		0.8845117

				352.9		0.8845117

				352.92		0.8845117

				352.94		0.8806317

				352.96		0.8806317

				352.98		0.8806317

				353		0.8806317

				353.02		0.8806317

				353.05		0.8806317

				353.07		0.8806317

				353.09		0.8806317

				353.11		0.8806317

				353.13		0.8806317

				353.15		0.8806317

				353.17		0.8806317

				353.19		0.8806317

				353.22		0.8806317

				353.24		0.8806317

				353.26		0.8806317

				353.28		0.8806317

				353.3		0.8806317

				353.32		0.8806317

				353.34		0.8806317

				353.36		0.8806317

				353.39		0.8845117

				353.41		0.8806317

				353.43		0.8845117

				353.45		0.8806317

				353.47		0.8806317

				353.49		0.8845117

				353.51		0.8845117

				353.53		0.8845117

				353.56		0.8845117

				353.58		0.8845117

				353.6		0.8845117

				353.62		0.8845117

				353.64		0.8845117

				353.66		0.8845117

				353.68		0.8845117

				353.7		0.8845117

				353.72		0.8845117

				353.75		0.8845117

				353.77		0.8845117

				353.79		0.8845117

				353.81		0.8845117

				353.83		0.8806317

				353.85		0.8845117

				353.87		0.8806317

				353.89		0.8845117

				353.92		0.8845117

				353.94		0.8845117

				353.96		0.8845117

				353.98		0.8845117

				354		0.8845117

				354.02		0.8845117

				354.04		0.8845117

				354.06		0.8845117

				354.09		0.8845117

				354.11		0.8845117

				354.13		0.8845117

				354.15		0.8845117

				354.17		0.8845117

				354.19		0.8845117

				354.21		0.8845117

				354.23		0.8845117

				354.25		0.8845117

				354.28		0.8845117

				354.3		0.8845117

				354.32		0.8845117

				354.34		0.8845117

				354.36		0.8845117

				354.38		0.8845117

				354.4		0.8845117

				354.42		0.8845117

				354.45		0.8845117

				354.47		0.8845117

				354.49		0.8845117

				354.51		0.8845117

				354.53		0.8883918

				354.55		0.8883918

				354.57		0.8883918

				354.59		0.8883918

				354.62		0.8883918

				354.64		0.8883918

				354.66		0.8883918

				354.68		0.8883918

				354.7		0.8883918

				354.72		0.8883918

				354.74		0.8883918

				354.76		0.8883918

				354.78		0.8883918

				354.81		0.8883918

				354.83		0.8883918

				354.85		0.8883918

				354.87		0.8883918

				354.89		0.8883918

				354.91		0.8883918

				354.93		0.8883918

				354.95		0.8883918

				354.98		0.8883918

				355		0.8883918

				355.02		0.8883918

				355.04		0.8883918

				355.06		0.8883918

				355.08		0.8883918

				355.1		0.8883918

				355.12		0.8883918

				355.14		0.8883918

				355.17		0.8883918

				355.19		0.8883918

				355.21		0.8883918

				355.23		0.8883918

				355.25		0.8883918

				355.27		0.8883918

				355.29		0.8883918

				355.31		0.8883918

				355.34		0.8883918

				355.36		0.8883918

				355.38		0.8883918

				355.4		0.8883918

				355.42		0.8883918

				355.44		0.8883918

				355.46		0.8883918

				355.48		0.8845117

				355.5		0.8883918

				355.53		0.8883918

				355.55		0.8883918

				355.57		0.8883918

				355.59		0.8883918

				355.61		0.8883918

				355.63		0.8883918

				355.65		0.8883918

				355.67		0.8883918

				355.7		0.8883918

				355.72		0.8883918

				355.74		0.8883918

				355.76		0.8883918

				355.78		0.8883918

				355.8		0.8883918

				355.82		0.8883918

				355.84		0.8883918

				355.87		0.8883918

				355.89		0.8883918

				355.91		0.8883918

				355.93		0.8883918

				355.95		0.8883918

				355.97		0.8883918

				355.99		0.8883918

				356.01		0.8883918

				356.03		0.8883918

				356.06		0.8883918

				356.08		0.8883918

				356.1		0.8883918

				356.12		0.8883918

				356.14		0.8883918

				356.16		0.8883918

				356.18		0.8883918

				356.2		0.8883918

				356.23		0.8883918

				356.25		0.8883918

				356.27		0.8883918

				356.29		0.8883918

				356.31		0.8883918

				356.33		0.8883918

				356.35		0.8883918

				356.37		0.8883918

				356.4		0.8883918

				356.42		0.8883918

				356.44		0.8883918

				356.46		0.8883918

				356.48		0.8883918

				356.5		0.8883918

				356.52		0.8883918

				356.54		0.8883918

				356.57		0.8883918

				356.59		0.8883918

				356.61		0.8883918

				356.63		0.8883918

				356.65		0.8883918

				356.67		0.8883918

				356.69		0.8883918

				356.71		0.8883918

				356.74		0.8883918

				356.76		0.8883918

				356.78		0.8883918

				356.8		0.8883918

				356.82		0.8883918

				356.84		0.8883918

				356.86		0.8883918

				356.88		0.8883918

				356.91		0.8883918

				356.93		0.8883918

				356.95		0.8883918

				356.97		0.8883918

				356.99		0.8883918

				357.01		0.8883918

				357.03		0.8883918

				357.05		0.8883918

				357.08		0.8883918

				357.1		0.8883918

				357.12		0.8883918

				357.14		0.8883918

				357.16		0.8883918

				357.18		0.8883918

				357.2		0.8883918

				357.22		0.8883918

				357.25		0.8883918

				357.27		0.8883918

				357.29		0.8883918

				357.31		0.8883918

				357.33		0.8883918

				357.35		0.8883918

				357.37		0.8883918

				357.39		0.8883918

				357.41		0.8883918

				357.44		0.8883918

				357.46		0.8883918

				357.48		0.8883918

				357.5		0.8883918

				357.52		0.8883918

				357.54		0.8883918

				357.56		0.8883918

				357.58		0.8883918

				357.61		0.8883918

				357.63		0.8883918

				357.65		0.8883918

				357.67		0.8883918

				357.69		0.8883918

				357.71		0.8883918

				357.73		0.8883918

				357.75		0.8883918

				357.78		0.8883918

				357.8		0.8883918

				357.82		0.8883918

				357.84		0.8845117

				357.86		0.8845117

				357.88		0.8845117

				357.9		0.8845117

				357.92		0.8845117

				357.94		0.8845117

				357.97		0.8845117

				357.99		0.8845117

				358.01		0.8845117

				358.03		0.8845117

				358.05		0.8845117

				358.07		0.8845117

				358.09		0.8845117

				358.11		0.8845117

				358.14		0.8845117

				358.16		0.8845117

				358.18		0.8845117

				358.2		0.8845117

				358.22		0.8845117

				358.24		0.8845117

				358.26		0.8845117

				358.28		0.8845117

				358.3		0.8845117

				358.33		0.8845117

				358.35		0.8845117

				358.37		0.8845117

				358.39		0.8845117

				358.41		0.8845117

				358.43		0.8845117

				358.45		0.8845117

				358.47		0.8845117

				358.5		0.8845117

				358.52		0.8845117

				358.54		0.8845117

				358.56		0.8845117

				358.58		0.8845117

				358.6		0.8845117

				358.62		0.8845117

				358.64		0.8845117

				358.67		0.8845117

				358.69		0.8845117

				358.71		0.8845117

				358.73		0.8845117

				358.75		0.8845117

				358.77		0.8845117

				358.79		0.8845117

				358.81		0.8845117

				358.84		0.8845117

				358.86		0.8845117

				358.88		0.8845117

				358.9		0.8845117

				358.92		0.8845117

				358.94		0.8845117

				358.96		0.8845117

				358.98		0.8845117

				359.01		0.8845117

				359.03		0.8845117

				359.05		0.8845117

				359.07		0.8845117

				359.09		0.8806317

				359.11		0.8806317

				359.13		0.8845117

				359.15		0.8806317

				359.17		0.8806317

				359.2		0.8806317

				359.22		0.8806317

				359.24		0.8806317

				359.26		0.8806317

				359.28		0.8806317

				359.3		0.8806317

				359.32		0.8806317

				359.34		0.8806317

				359.37		0.8806317

				359.39		0.8806317

				359.41		0.8806317

				359.43		0.8806317

				359.45		0.8806317

				359.47		0.8806317

				359.49		0.8806317

				359.51		0.8806317

				359.54		0.8806317

				359.56		0.8806317

				359.58		0.8806317

				359.6		0.8806317

				359.62		0.8806317

				359.64		0.8806317

				359.66		0.8806317

				359.68		0.8806317

				359.71		0.8806317

				359.73		0.8806317

				359.75		0.8806317

				359.77		0.8806317

				359.79		0.8806317

				359.81		0.8806317

				359.83		0.8806317

				359.85		0.8806317

				359.87		0.8806317

				359.9		0.8806317

				359.92		0.8806317

				359.94		0.8806317

				359.96		0.8806317

				359.98		0.8806317

				360		0.8806317

				360.02		0.8806317

				360.04		0.8806317

				360.07		0.8806317

				360.09		0.8806317

				360.11		0.8806317

				360.13		0.8806317

				360.15		0.8806317

				360.17		0.8806317

				360.19		0.8806317

				360.21		0.8806317

				360.24		0.8806317

				360.26		0.8806317

				360.28		0.8806317

				360.3		0.8806317

				360.32		0.8806317

				360.34		0.8806317

				360.36		0.8806317

				360.38		0.8806317

				360.4		0.8806317

				360.43		0.8767516

				360.45		0.8767516

				360.47		0.8767516

				360.49		0.8767516

				360.51		0.8806317

				360.53		0.8767516

				360.55		0.8806317

				360.57		0.8767516

				360.6		0.8806317

				360.62		0.8767516

				360.64		0.8767516

				360.66		0.8806317

				360.68		0.8806317

				360.7		0.8767516

				360.72		0.8806317

				360.74		0.8806317

				360.76		0.8806317

				360.79		0.8806317

				360.81		0.8806317

				360.83		0.8806317

				360.85		0.8806317

				360.87		0.8806317

				360.89		0.8806317

				360.91		0.8806317

				360.93		0.8806317

				360.96		0.8806317

				360.98		0.8806317

				361		0.8806317

				361.02		0.8806317

				361.04		0.8806317

				361.06		0.8806317

				361.08		0.8806317

				361.1		0.8806317

				361.13		0.8806317

				361.15		0.8806317

				361.17		0.8806317

				361.19		0.8806317

				361.21		0.8806317

				361.23		0.8806317

				361.25		0.8806317

				361.27		0.8806317

				361.29		0.8806317

				361.32		0.8806317

				361.34		0.8806317

				361.36		0.8806317

				361.38		0.8806317

				361.4		0.8806317

				361.42		0.8806317

				361.44		0.8806317

				361.46		0.8806317

				361.49		0.8806317

				361.51		0.8806317

				361.53		0.8806317

				361.55		0.8806317

				361.57		0.8806317

				361.59		0.8806317

				361.61		0.8806317

				361.63		0.8806317

				361.66		0.8806317

				361.68		0.8806317

				361.7		0.8806317

				361.72		0.8767516

				361.74		0.8767516

				361.76		0.8767516

				361.78		0.8767516

				361.8		0.8767516

				361.82		0.8806317

				361.85		0.8806317

				361.87		0.8806317

				361.89		0.8767516

				361.91		0.8806317

				361.93		0.8806317

				361.95		0.8767516

				361.97		0.8767516

				361.99		0.8767516

				362.02		0.8806317

				362.04		0.8806317

				362.06		0.8806317

				362.08		0.8767516

				362.1		0.8806317

				362.12		0.8806317

				362.14		0.8767516

				362.16		0.8806317

				362.18		0.8767516

				362.21		0.8806317

				362.23		0.8767516

				362.25		0.8806317

				362.27		0.8806317

				362.29		0.8767516

				362.31		0.8806317

				362.33		0.8806317

				362.35		0.8806317

				362.38		0.8806317

				362.4		0.8806317

				362.42		0.8767516

				362.44		0.8806317

				362.46		0.8806317

				362.48		0.8806317

				362.5		0.8806317

				362.52		0.8806317

				362.55		0.8806317

				362.57		0.8806317

				362.59		0.8806317

				362.61		0.8806317

				362.63		0.8806317

				362.65		0.8806317

				362.67		0.8806317

				362.69		0.8806317

				362.71		0.8806317

				362.74		0.8767516

				362.76		0.8806317

				362.78		0.8767516

				362.8		0.8806317

				362.82		0.8767516

				362.84		0.8806317

				362.86		0.8806317

				362.88		0.8806317

				362.91		0.8806317

				362.93		0.8806317

				362.95		0.8806317

				362.97		0.8806317

				362.99		0.8806317

				363.01		0.8806317

				363.03		0.8806317

				363.05		0.8806317

				363.08		0.8806317

				363.1		0.8806317

				363.12		0.8806317

				363.14		0.8806317

				363.16		0.8806317

				363.18		0.8806317

				363.2		0.8806317

				363.22		0.8806317

				363.24		0.8806317

				363.27		0.8806317

				363.29		0.8806317

				363.31		0.8806317

				363.33		0.8806317

				363.35		0.8806317

				363.37		0.8806317

				363.39		0.8806317

				363.41		0.8806317

				363.44		0.8806317

				363.46		0.8806317

				363.48		0.8806317

				363.5		0.8806317

				363.52		0.8806317

				363.54		0.8806317

				363.56		0.8806317

				363.58		0.8806317

				363.61		0.8806317

				363.63		0.8806317

				363.65		0.8806317

				363.67		0.8806317

				363.69		0.8806317

				363.71		0.8806317

				363.73		0.8806317

				363.75		0.8806317

				363.78		0.8806317

				363.8		0.8806317

				363.82		0.8806317

				363.84		0.8806317

				363.86		0.8806317

				363.88		0.8806317

				363.9		0.8806317

				363.92		0.8806317

				363.94		0.8806317

				363.97		0.8806317

				363.99		0.8806317

				364.01		0.8806317

				364.03		0.8806317

				364.05		0.8806317

				364.07		0.8806317

				364.09		0.8806317

				364.11		0.8806317

				364.14		0.8767516

				364.16		0.8806317

				364.18		0.8806317

				364.2		0.8806317

				364.22		0.8806317

				364.24		0.8806317

				364.26		0.8806317

				364.28		0.8806317

				364.3		0.8806317

				364.33		0.8806317

				364.35		0.8806317

				364.37		0.8806317

				364.39		0.8806317

				364.41		0.8806317

				364.43		0.8806317

				364.45		0.8806317

				364.47		0.8806317

				364.5		0.8806317

				364.52		0.8806317

				364.54		0.8806317

				364.56		0.8806317

				364.58		0.8806317

				364.6		0.8806317

				364.62		0.8767516

				364.64		0.8767516

				364.67		0.8767516

				364.69		0.8767516

				364.71		0.8767516

				364.73		0.8767516

				364.75		0.8767516

				364.77		0.8767516

				364.79		0.8767516

				364.81		0.8767516

				364.84		0.8767516

				364.86		0.8767516

				364.88		0.8767516

				364.9		0.8767516

				364.92		0.8767516

				364.94		0.8767516

				364.96		0.8767516

				364.98		0.8767516

				365		0.8767516

				365.03		0.8767516

				365.05		0.8728716

				365.07		0.8728716

				365.09		0.8728716

				365.11		0.8728716

				365.13		0.8728716

				365.15		0.8728716

				365.17		0.8728716

				365.2		0.8728716

				365.22		0.8728716

				365.24		0.8728716

				365.26		0.8728716

				365.28		0.8728716

				365.3		0.8728716

				365.32		0.8728716

				365.34		0.8728716

				365.37		0.8728716

				365.39		0.8728716

				365.41		0.8728716

				365.43		0.8728716

				365.45		0.8728716

				365.47		0.8728716

				365.49		0.8728716

				365.51		0.8728716

				365.53		0.8728716

				365.56		0.8728716

				365.58		0.8689916

				365.6		0.8689916

				365.62		0.8689916

				365.64		0.8689916

				365.66		0.8689916

				365.68		0.8689916

				365.7		0.8689916

				365.73		0.8689916

				365.75		0.8689916

				365.77		0.8689916

				365.79		0.8689916

				365.81		0.8689916

				365.83		0.8689916

				365.85		0.8689916

				365.87		0.8689916

				365.9		0.8689916

				365.92		0.8689916

				365.94		0.8689916

				365.96		0.8689916

				365.98		0.8689916

				366		0.8689916

				366.02		0.8651115

				366.04		0.8651115

				366.06		0.8651115

				366.09		0.8651115

				366.11		0.8651115

				366.13		0.8651115

				366.15		0.8651115

				366.17		0.8651115

				366.19		0.8651115

				366.21		0.8689916

				366.23		0.8689916

				366.26		0.8651115

				366.28		0.8689916

				366.3		0.8689916

				366.32		0.8689916

				366.34		0.8689916

				366.36		0.8689916

				366.38		0.8651115

				366.4		0.8651115

				366.42		0.8651115

				366.45		0.8651115

				366.47		0.8651115

				366.49		0.8651115

				366.51		0.8651115

				366.53		0.8651115

				366.55		0.8651115

				366.57		0.8651115

				366.59		0.8651115

				366.62		0.8651115

				366.64		0.8651115

				366.66		0.8651115

				366.68		0.8651115

				366.7		0.8651115

				366.72		0.8689916

				366.74		0.8651115

				366.76		0.8689916

				366.78		0.8689916

				366.81		0.8689916

				366.83		0.8689916

				366.85		0.8689916

				366.87		0.8651115

				366.89		0.8651115

				366.91		0.8651115

				366.93		0.8651115

				366.95		0.8651115

				366.98		0.8651115

				367		0.8651115

				367.02		0.8651115

				367.04		0.8651115

				367.06		0.8651115

				367.08		0.8651115

				367.1		0.8651115

				367.12		0.8651115

				367.15		0.8689916

				367.17		0.8689916

				367.19		0.8651115

				367.21		0.8651115

				367.23		0.8651115

				367.25		0.8651115

				367.27		0.8651115

				367.29		0.8651115

				367.31		0.8651115

				367.34		0.8651115

				367.36		0.8651115

				367.38		0.8651115

				367.4		0.8651115

				367.42		0.8651115

				367.44		0.8651115

				367.46		0.8651115

				367.48		0.8651115

				367.51		0.8651115

				367.53		0.8651115

				367.55		0.8651115

				367.57		0.8651115

				367.59		0.8651115

				367.61		0.8651115

				367.63		0.8651115

				367.65		0.8651115

				367.67		0.8651115

				367.7		0.8651115

				367.72		0.8651115

				367.74		0.8651115

				367.76		0.8651115

				367.78		0.8689916

				367.8		0.8651115

				367.82		0.8651115

				367.84		0.8651115

				367.87		0.8651115

				367.89		0.8651115

				367.91		0.8651115

				367.93		0.8651115

				367.95		0.8651115

				367.97		0.8651115

				367.99		0.8651115

				368.01		0.8651115

				368.04		0.8651115

				368.06		0.8651115

				368.08		0.8651115

				368.1		0.8651115

				368.12		0.8651115

				368.14		0.8651115

				368.16		0.8651115

				368.18		0.8651115

				368.21		0.8651115

				368.23		0.8651115

				368.25		0.8651115

				368.27		0.8651115

				368.29		0.8651115

				368.31		0.8651115

				368.33		0.8651115

				368.35		0.8651115

				368.38		0.8651115

				368.4		0.8651115

				368.42		0.8651115

				368.44		0.8651115

				368.46		0.8651115

				368.48		0.8651115

				368.5		0.8651115

				368.52		0.8651115

				368.55		0.8651115

				368.57		0.8651115

				368.59		0.8651115

				368.61		0.8651115

				368.63		0.8651115

				368.65		0.8651115

				368.67		0.8651115

				368.69		0.8651115

				368.72		0.8651115

				368.74		0.8651115

				368.76		0.8651115

				368.78		0.8651115

				368.8		0.8651115

				368.82		0.8612315

				368.84		0.8651115

				368.86		0.8651115

				368.89		0.8651115

				368.91		0.8651115

				368.93		0.8651115

				368.95		0.8651115

				368.97		0.8651115

				368.99		0.8651115

				369.01		0.8651115

				369.03		0.8651115

				369.06		0.8651115

				369.08		0.8651115

				369.1		0.8651115

				369.12		0.8612315

				369.14		0.8612315

				369.16		0.8612315

				369.18		0.8612315

				369.2		0.8612315

				369.22		0.8612315

				369.25		0.8612315

				369.27		0.8612315

				369.29		0.8612315

				369.31		0.8612315

				369.33		0.8612315

				369.35		0.8612315

				369.37		0.8612315

				369.39		0.8612315

				369.42		0.8612315

				369.44		0.8651115

				369.46		0.8651115

				369.48		0.8651115

				369.5		0.8651115

				369.52		0.8651115

				369.54		0.8651115

				369.56		0.8651115

				369.59		0.8651115

				369.61		0.8651115

				369.63		0.8651115

				369.65		0.8651115

				369.67		0.8651115

				369.69		0.8651115

				369.71		0.8689916

				369.73		0.8689916

				369.75		0.8689916

				369.78		0.8651115

				369.8		0.8689916

				369.82		0.8651115

				369.84		0.8651115

				369.86		0.8689916

				369.88		0.8651115

				369.9		0.8651115

				369.92		0.8651115

				369.95		0.8689916

				369.97		0.8689916

				369.99		0.8689916

				370.01		0.8689916

				370.03		0.8689916

				370.05		0.8689916

				370.07		0.8689916

				370.09		0.8689916

				370.12		0.8689916

				370.14		0.8689916

				370.16		0.8689916

				370.18		0.8689916

				370.2		0.8689916

				370.22		0.8689916

				370.24		0.8689916

				370.26		0.8689916

				370.29		0.8689916

				370.31		0.8689916

				370.33		0.8689916

				370.35		0.8689916

				370.37		0.8689916

				370.39		0.8689916

				370.41		0.8689916

				370.43		0.8689916

				370.45		0.8689916

				370.48		0.8689916

				370.5		0.8689916

				370.52		0.8689916

				370.54		0.8689916

				370.56		0.8689916

				370.58		0.8689916

				370.6		0.8689916

				370.62		0.8689916

				370.65		0.8689916

				370.67		0.8689916

				370.69		0.8689916

				370.71		0.8689916

				370.73		0.8689916

				370.75		0.8689916

				370.77		0.8689916

				370.79		0.8689916

				370.82		0.8689916

				370.84		0.8689916

				370.86		0.8689916

				370.88		0.8689916

				370.9		0.8689916

				370.92		0.8689916

				370.94		0.8689916

				370.96		0.8651115

				370.99		0.8651115

				371.01		0.8651115

				371.03		0.8651115

				371.05		0.8689916

				371.07		0.8689916

				371.09		0.8689916

				371.11		0.8689916

				371.13		0.8689916

				371.16		0.8689916

				371.18		0.8689916

				371.2		0.8689916

				371.22		0.8689916

				371.24		0.8689916

				371.26		0.8689916

				371.28		0.8689916

				371.3		0.8689916

				371.33		0.8689916

				371.35		0.8689916

				371.37		0.8689916

				371.39		0.8689916

				371.41		0.8689916

				371.43		0.8689916

				371.45		0.8689916

				371.47		0.8689916

				371.5		0.8689916

				371.52		0.8689916

				371.54		0.8651115

				371.56		0.8689916

				371.58		0.8651115

				371.6		0.8651115

				371.62		0.8689916

				371.64		0.8651115

				371.67		0.8651115

				371.69		0.8651115

				371.71		0.8651115

				371.73		0.8651115

				371.75		0.8651115

				371.77		0.8651115

				371.79		0.8651115

				371.81		0.8651115

				371.84		0.8651115

				371.86		0.8651115

				371.88		0.8651115

				371.9		0.8651115

				371.92		0.8651115

				371.94		0.8651115

				371.96		0.8651115

				371.98		0.8651115

				372.01		0.8651115

				372.03		0.8651115

				372.05		0.8651115

				372.07		0.8651115

				372.09		0.8651115

				372.11		0.8651115

				372.13		0.8651115

				372.15		0.8651115

				372.18		0.8651115

				372.2		0.8651115

				372.22		0.8651115

				372.24		0.8651115

				372.26		0.8651115

				372.28		0.8651115

				372.3		0.8651115

				372.32		0.8651115

				372.35		0.8651115

				372.37		0.8651115

				372.39		0.8651115

				372.41		0.8651115

				372.43		0.8651115

				372.45		0.8651115

				372.47		0.8651115

				372.49		0.8651115

				372.51		0.8651115

				372.54		0.8651115

				372.56		0.8651115

				372.58		0.8651115

				372.6		0.8651115

				372.62		0.8651115

				372.64		0.8651115

				372.66		0.8651115

				372.68		0.8651115

				372.71		0.8651115

				372.73		0.8612315

				372.75		0.8651115

				372.77		0.8651115

				372.79		0.8651115

				372.81		0.8612315

				372.83		0.8612315

				372.85		0.8612315

				372.88		0.8612315

				372.9		0.8612315

				372.92		0.8651115

				372.94		0.8651115

				372.96		0.8651115

				372.98		0.8651115

				373		0.8651115

				373.02		0.8651115

				373.05		0.8651115

				373.07		0.8651115

				373.09		0.8651115

				373.11		0.8651115

				373.13		0.8651115

				373.15		0.8651115

				373.17		0.8651115

				373.19		0.8651115

				373.22		0.8651115

				373.24		0.8651115

				373.26		0.8651115

				373.28		0.8651115

				373.3		0.8651115

				373.32		0.8651115

				373.34		0.8651115

				373.36		0.8651115

				373.39		0.8651115

				373.41		0.8651115

				373.43		0.8651115

				373.45		0.8651115

				373.47		0.8651115

				373.49		0.8651115

				373.51		0.8651115

				373.53		0.8651115

				373.56		0.8651115

				373.58		0.8651115

				373.6		0.8651115

				373.62		0.8651115

				373.64		0.8651115

				373.66		0.8689916

				373.68		0.8689916

				373.7		0.8689916

				373.73		0.8651115

				373.75		0.8651115

				373.77		0.8651115

				373.79		0.8689916

				373.81		0.8689916

				373.83		0.8689916

				373.85		0.8689916

				373.87		0.8689916

				373.9		0.8689916

				373.92		0.8689916

				373.94		0.8689916

				373.96		0.8689916

				373.98		0.8689916

				374		0.8689916

				374.02		0.8689916

				374.04		0.8689916

				374.06		0.8689916

				374.09		0.8689916

				374.11		0.8689916

				374.13		0.8689916

				374.15		0.8689916

				374.17		0.8689916

				374.19		0.8689916

				374.21		0.8689916

				374.23		0.8689916

				374.26		0.8689916

				374.28		0.8689916

				374.3		0.8689916

				374.32		0.8651115

				374.34		0.8651115

				374.36		0.8651115

				374.38		0.8689916

				374.4		0.8689916

				374.43		0.8689916

				374.45		0.8689916

				374.47		0.8689916

				374.49		0.8689916

				374.51		0.8689916

				374.53		0.8689916

				374.55		0.8689916

				374.57		0.8689916

				374.6		0.8728716

				374.62		0.8689916

				374.64		0.8689916

				374.66		0.8689916

				374.68		0.8689916

				374.7		0.8689916

				374.72		0.8689916

				374.74		0.8689916

				374.77		0.8689916

				374.79		0.8689916

				374.81		0.8689916

				374.83		0.8689916

				374.85		0.8689916

				374.87		0.8728716

				374.89		0.8689916

				374.91		0.8689916

				374.94		0.8728716

				374.96		0.8728716

				374.98		0.8728716

				375		0.8689916

				375.02		0.8689916

				375.04		0.8689916

				375.06		0.8689916

				375.08		0.8689916

				375.11		0.8689916

				375.13		0.8689916

				375.15		0.8689916

				375.17		0.8689916

				375.19		0.8689916

				375.21		0.8689916

				375.23		0.8689916

				375.25		0.8689916

				375.28		0.8689916

				375.3		0.8689916

				375.32		0.8689916

				375.34		0.8689916

				375.36		0.8689916

				375.38		0.8689916

				375.4		0.8689916

				375.42		0.8689916

				375.45		0.8689916

				375.47		0.8689916

				375.49		0.8689916

				375.51		0.8689916

				375.53		0.8689916

				375.55		0.8689916

				375.57		0.8689916

				375.59		0.8689916

				375.62		0.8689916

				375.64		0.8689916

				375.66		0.8689916

				375.68		0.8689916

				375.7		0.8689916

				375.72		0.8689916

				375.74		0.8689916

				375.76		0.8689916

				375.79		0.8689916

				375.81		0.8689916

				375.83		0.8689916

				375.85		0.8689916

				375.87		0.8689916

				375.89		0.8689916

				375.91		0.8689916

				375.93		0.8689916

				375.96		0.8689916

				375.98		0.8689916

				376		0.8689916

				376.02		0.8689916

				376.04		0.8689916

				376.06		0.8689916

				376.08		0.8689916

				376.1		0.8689916

				376.13		0.8651115

				376.15		0.8651115

				376.17		0.8651115

				376.19		0.8651115

				376.21		0.8651115

				376.23		0.8651115

				376.25		0.8651115

				376.27		0.8651115

				376.3		0.8651115

				376.32		0.8651115

				376.34		0.8651115

				376.36		0.8651115

				376.38		0.8651115

				376.4		0.8651115

				376.42		0.8651115

				376.44		0.8651115

				376.47		0.8689916

				376.49		0.8651115

				376.51		0.8651115

				376.53		0.8651115

				376.55		0.8651115

				376.57		0.8651115

				376.59		0.8651115

				376.61		0.8651115

				376.64		0.8651115

				376.66		0.8651115

				376.68		0.8651115

				376.7		0.8651115

				376.72		0.8651115

				376.74		0.8651115

				376.76		0.8651115

				376.78		0.8651115

				376.81		0.8651115

				376.83		0.8651115

				376.85		0.8651115

				376.87		0.8651115

				376.89		0.8651115

				376.91		0.8651115

				376.93		0.8651115

				376.95		0.8651115

				376.98		0.8651115

				377		0.8651115

				377.02		0.8651115

				377.04		0.8651115

				377.06		0.8689916

				377.08		0.8651115

				377.1		0.8689916

				377.12		0.8689916

				377.14		0.8651115

				377.17		0.8689916

				377.19		0.8689916

				377.21		0.8651115

				377.23		0.8651115

				377.25		0.8651115

				377.27		0.8651115

				377.29		0.8651115

				377.31		0.8651115

				377.34		0.8651115

				377.36		0.8651115

				377.38		0.8651115

				377.4		0.8689916

				377.42		0.8689916

				377.44		0.8689916

				377.46		0.8651115

				377.49		0.8651115

				377.51		0.8689916

				377.53		0.8689916

				377.55		0.8651115

				377.57		0.8651115

				377.59		0.8651115

				377.61		0.8689916

				377.63		0.8651115

				377.66		0.8651115

				377.68		0.8689916

				377.7		0.8689916

				377.72		0.8689916

				377.74		0.8689916

				377.76		0.8689916

				377.78		0.8689916

				377.8		0.8689916

				377.83		0.8689916

				377.85		0.8689916

				377.87		0.8689916

				377.89		0.8689916

				377.91		0.8689916

				377.93		0.8689916

				377.95		0.8689916

				377.97		0.8689916

				378		0.8689916

				378.02		0.8689916

				378.04		0.8689916

				378.06		0.8689916

				378.08		0.8689916

				378.1		0.8651115

				378.12		0.8689916

				378.14		0.8651115

				378.17		0.8651115

				378.19		0.8689916

				378.21		0.8689916

				378.23		0.8689916

				378.25		0.8651115

				378.27		0.8689916

				378.29		0.8689916

				378.31		0.8689916

				378.34		0.8689916

				378.36		0.8689916

				378.38		0.8689916

				378.4		0.8689916

				378.42		0.8689916

				378.44		0.8689916

				378.46		0.8689916

				378.48		0.8689916

				378.51		0.8689916

				378.53		0.8689916

				378.55		0.8689916

				378.57		0.8689916

				378.59		0.8689916

				378.61		0.8689916

				378.63		0.8689916

				378.65		0.8689916

				378.68		0.8689916

				378.7		0.8689916

				378.72		0.8689916

				378.74		0.8689916

				378.76		0.8689916

				378.78		0.8689916

				378.8		0.8689916

				378.82		0.8689916

				378.85		0.8689916

				378.87		0.8689916

				378.89		0.8689916

				378.91		0.8689916

				378.93		0.8689916

				378.95		0.8689916

				378.97		0.8689916

				378.99		0.8689916

				379.02		0.8651115

				379.04		0.8689916

				379.06		0.8689916

				379.08		0.8689916

				379.1		0.8689916

				379.12		0.8689916

				379.14		0.8651115

				379.16		0.8651115

				379.19		0.8651115

				379.21		0.8651115

				379.23		0.8651115

				379.25		0.8689916

				379.27		0.8651115

				379.29		0.8689916

				379.31		0.8689916

				379.33		0.8689916

				379.36		0.8689916

				379.38		0.8689916

				379.4		0.8689916

				379.42		0.8689916

				379.44		0.8689916

				379.46		0.8689916

				379.48		0.8689916

				379.5		0.8689916

				379.53		0.8689916

				379.55		0.8689916

				379.57		0.8689916

				379.59		0.8689916

				379.61		0.8651115

				379.63		0.8651115

				379.65		0.8689916

				379.67		0.8689916

				379.7		0.8689916

				379.72		0.8689916

				379.74		0.8689916

				379.76		0.8689916

				379.78		0.8689916

				379.8		0.8689916

				379.82		0.8689916

				379.84		0.8689916

				379.87		0.8651115

				379.89		0.8689916

				379.91		0.8689916

				379.93		0.8689916

				379.95		0.8689916

				379.97		0.8689916

				379.99		0.8689916

				380.01		0.8689916

				380.04		0.8689916

				380.06		0.8689916

				380.08		0.8689916

				380.1		0.8689916

				380.12		0.8689916

				380.14		0.8689916

				380.16		0.8689916

				380.18		0.8689916

				380.21		0.8689916

				380.23		0.8689916

				380.25		0.8689916

				380.27		0.8689916

				380.29		0.8689916

				380.31		0.8689916

				380.33		0.8689916

				380.35		0.8689916

				380.38		0.8689916

				380.4		0.8689916

				380.42		0.8689916

				380.44		0.8689916

				380.46		0.8689916

				380.48		0.8689916

				380.5		0.8689916

				380.52		0.8689916

				380.55		0.8689916

				380.57		0.8689916

				380.59		0.8689916

				380.61		0.8689916

				380.63		0.8689916

				380.65		0.8689916

				380.67		0.8689916

				380.7		0.8689916

				380.72		0.8689916

				380.74		0.8689916

				380.76		0.8689916

				380.78		0.8689916

				380.8		0.8689916

				380.82		0.8689916

				380.84		0.8689916

				380.87		0.8689916

				380.89		0.8689916

				380.91		0.8689916

				380.93		0.8689916

				380.95		0.8689916

				380.97		0.8689916

				380.99		0.8689916

				381.01		0.8689916

				381.04		0.8689916

				381.06		0.8689916

				381.08		0.8689916

				381.1		0.8689916

				381.12		0.8689916

				381.14		0.8689916

				381.16		0.8689916

				381.18		0.8689916

				381.21		0.8689916

				381.23		0.8689916

				381.25		0.8689916

				381.27		0.8689916

				381.29		0.8689916

				381.31		0.8689916

				381.33		0.8689916

				381.35		0.8689916

				381.38		0.8689916

				381.4		0.8689916

				381.42		0.8689916

				381.44		0.8689916

				381.46		0.8728716

				381.48		0.8689916

				381.5		0.8728716

				381.52		0.8728716

				381.55		0.8728716

				381.57		0.8728716

				381.59		0.8728716

				381.61		0.8728716

				381.63		0.8728716

				381.65		0.8728716

				381.67		0.8728716

				381.69		0.8728716

				381.72		0.8728716

				381.74		0.8728716

				381.76		0.8728716

				381.78		0.8728716

				381.8		0.8728716

				381.82		0.8728716

				381.84		0.8728716

				381.86		0.8728716

				381.89		0.8728716

				381.91		0.8728716

				381.93		0.8728716

				381.95		0.8728716

				381.97		0.8728716

				381.99		0.8728716

				382.01		0.8728716

				382.03		0.8728716

				382.05		0.8728716

				382.08		0.8728716

				382.1		0.8728716

				382.12		0.8728716

				382.14		0.8728716

				382.16		0.8728716

				382.18		0.8728716

				382.2		0.8728716

				382.22		0.8728716

				382.25		0.8728716

				382.27		0.8728716

				382.29		0.8728716

				382.31		0.8728716

				382.33		0.8728716

				382.35		0.8728716

				382.37		0.8728716

				382.39		0.8728716

				382.42		0.8728716

				382.44		0.8728716

				382.46		0.8728716

				382.48		0.8728716

				382.5		0.8728716

				382.52		0.8728716

				382.54		0.8728716

				382.56		0.8728716

				382.59		0.8728716

				382.61		0.8728716

				382.63		0.8728716

				382.65		0.8728716

				382.67		0.8728716

				382.69		0.8767516

				382.71		0.8728716

				382.73		0.8728716

				382.76		0.8767516

				382.78		0.8767516

				382.8		0.8767516

				382.82		0.8728716

				382.84		0.8767516

				382.86		0.8767516

				382.88		0.8728716

				382.9		0.8767516

				382.93		0.8767516

				382.95		0.8767516

				382.97		0.8767516

				382.99		0.8767516

				383.01		0.8767516

				383.03		0.8767516

				383.05		0.8767516

				383.07		0.8767516

				383.1		0.8767516

				383.12		0.8767516

				383.14		0.8767516

				383.16		0.8767516

				383.18		0.8767516

				383.2		0.8767516

				383.22		0.8767516

				383.24		0.8728716

				383.27		0.8767516

				383.29		0.8728716

				383.31		0.8728716

				383.33		0.8728716

				383.35		0.8728716

				383.37		0.8728716

				383.39		0.8728716

				383.41		0.8728716

				383.44		0.8767516

				383.46		0.8728716

				383.48		0.8728716

				383.5		0.8728716

				383.52		0.8728716

				383.54		0.8728716

				383.56		0.8728716

				383.58		0.8728716

				383.61		0.8728716

				383.63		0.8728716

				383.65		0.8728716

				383.67		0.8728716

				383.69		0.8728716

				383.71		0.8728716

				383.73		0.8728716

				383.75		0.8689916

				383.78		0.8689916

				383.8		0.8689916

				383.82		0.8689916

				383.84		0.8689916

				383.86		0.8689916

				383.88		0.8689916

				383.9		0.8689916

				383.92		0.8689916

				383.95		0.8689916

				383.97		0.8689916

				383.99		0.8689916

				384.01		0.8689916

				384.03		0.8689916

				384.05		0.8689916

				384.07		0.8689916

				384.09		0.8689916

				384.11		0.8689916

				384.14		0.8689916

				384.16		0.8689916

				384.18		0.8651115

				384.2		0.8651115

				384.22		0.8651115

				384.24		0.8651115

				384.26		0.8651115

				384.28		0.8651115

				384.31		0.8689916

				384.33		0.8651115

				384.35		0.8651115

				384.37		0.8651115

				384.39		0.8651115

				384.41		0.8651115

				384.43		0.8651115

				384.45		0.8651115

				384.48		0.8651115

				384.5		0.8651115

				384.52		0.8651115

				384.54		0.8651115

				384.56		0.8651115

				384.58		0.8651115

				384.6		0.8651115

				384.62		0.8651115

				384.65		0.8651115

				384.67		0.8651115

				384.69		0.8651115

				384.71		0.8651115

				384.73		0.8651115

				384.75		0.8651115

				384.77		0.8651115

				384.79		0.8651115

				384.82		0.8651115

				384.84		0.8651115

				384.86		0.8612315

				384.88		0.8612315

				384.9		0.8612315

				384.92		0.8612315

				384.94		0.8612315

				384.96		0.8651115

				384.99		0.8651115

				385.01		0.8612315

				385.03		0.8651115

				385.05		0.8651115

				385.07		0.8651115

				385.09		0.8651115

				385.11		0.8651115

				385.13		0.8651115

				385.16		0.8651115

				385.18		0.8651115

				385.2		0.8651115

				385.22		0.8651115

				385.24		0.8651115

				385.26		0.8612315

				385.28		0.8651115

				385.3		0.8612315

				385.33		0.8651115

				385.35		0.8651115

				385.37		0.8612315

				385.39		0.8651115

				385.41		0.8651115

				385.43		0.8651115

				385.45		0.8651115

				385.47		0.8651115

				385.5		0.8651115

				385.52		0.8651115

				385.54		0.8612315

				385.56		0.8651115

				385.58		0.8612315

				385.6		0.8612315

				385.62		0.8612315

				385.64		0.8612315

				385.67		0.8612315

				385.69		0.8651115

				385.71		0.8612315

				385.73		0.8612315

				385.75		0.8612315

				385.77		0.8612315

				385.79		0.8612315

				385.81		0.8651115

				385.84		0.8651115

				385.86		0.8651115

				385.88		0.8651115

				385.9		0.8651115

				385.92		0.8651115

				385.94		0.8651115

				385.96		0.8651115

				385.98		0.8612315

				386		0.8651115

				386.03		0.8651115

				386.05		0.8651115

				386.07		0.8651115

				386.09		0.8651115

				386.11		0.8651115

				386.13		0.8651115

				386.15		0.8651115

				386.17		0.8651115

				386.2		0.8651115

				386.22		0.8651115

				386.24		0.8651115

				386.26		0.8651115

				386.28		0.8651115

				386.3		0.8651115

				386.32		0.8651115

				386.34		0.8651115

				386.37		0.8651115

				386.39		0.8651115

				386.41		0.8651115

				386.43		0.8612315

				386.45		0.8651115

				386.47		0.8612315

				386.49		0.8612315

				386.51		0.8612315

				386.53		0.8651115

				386.56		0.8651115

				386.58		0.8612315

				386.6		0.8651115

				386.62		0.8651115

				386.64		0.8651115

				386.66		0.8651115

				386.68		0.8651115

				386.7		0.8651115

				386.73		0.8651115

				386.75		0.8651115

				386.77		0.8651115

				386.79		0.8651115

				386.81		0.8651115

				386.83		0.8612315

				386.85		0.8651115

				386.87		0.8651115

				386.9		0.8612315

				386.92		0.8651115

				386.94		0.8651115

				386.96		0.8651115

				386.98		0.8651115

				387		0.8651115

				387.02		0.8651115

				387.04		0.8651115

				387.07		0.8612315

				387.09		0.8612315

				387.11		0.8612315

				387.13		0.8612315

				387.15		0.8612315

				387.17		0.8612315

				387.19		0.8612315

				387.21		0.8612315

				387.23		0.8612315

				387.26		0.8612315

				387.28		0.8612315

				387.3		0.8612315

				387.32		0.8612315

				387.34		0.8612315

				387.36		0.8612315

				387.38		0.8612315

				387.4		0.8612315

				387.43		0.8612315

				387.45		0.8612315

				387.47		0.8612315

				387.49		0.8612315

				387.51		0.8612315

				387.53		0.8612315

				387.55		0.8612315

				387.57		0.8612315

				387.6		0.8612315

				387.62		0.8612315

				387.64		0.8612315

				387.66		0.8612315

				387.68		0.8612315

				387.7		0.8612315

				387.72		0.8612315

				387.74		0.8612315

				387.77		0.8612315

				387.79		0.8612315

				387.81		0.8612315

				387.83		0.8612315

				387.85		0.8612315

				387.87		0.8612315

				387.89		0.8612315

				387.91		0.8612315

				387.94		0.8612315

				387.96		0.8612315

				387.98		0.8612315

				388		0.8612315

				388.02		0.8612315

				388.04		0.8612315

				388.06		0.8612315

				388.08		0.8612315

				388.11		0.8573515

				388.13		0.8612315

				388.15		0.8612315

				388.17		0.8612315

				388.19		0.8573515

				388.21		0.8612315

				388.23		0.8573515

				388.25		0.8612315

				388.28		0.8612315

				388.3		0.8612315

				388.32		0.8612315

				388.34		0.8612315

				388.36		0.8612315

				388.38		0.8612315

				388.4		0.8612315

				388.42		0.8612315

				388.45		0.8612315

				388.47		0.8612315

				388.49		0.8612315

				388.51		0.8612315

				388.53		0.8612315

				388.55		0.8612315

				388.57		0.8612315

				388.59		0.8612315

				388.62		0.8612315

				388.64		0.8612315

				388.66		0.8612315

				388.68		0.8612315

				388.7		0.8612315

				388.72		0.8612315

				388.74		0.8612315

				388.76		0.8612315

				388.79		0.8651115

				388.81		0.8612315

				388.83		0.8612315

				388.85		0.8651115

				388.87		0.8651115

				388.89		0.8612315

				388.91		0.8612315

				388.93		0.8651115

				388.95		0.8612315

				388.98		0.8651115

				389		0.8651115

				389.02		0.8651115

				389.04		0.8651115

				389.06		0.8651115

				389.08		0.8651115

				389.1		0.8651115

				389.12		0.8651115

				389.15		0.8651115

				389.17		0.8651115

				389.19		0.8651115

				389.21		0.8651115

				389.23		0.8651115

				389.25		0.8651115

				389.27		0.8651115

				389.29		0.8651115

				389.32		0.8651115

				389.34		0.8651115

				389.36		0.8651115

				389.38		0.8651115

				389.4		0.8651115

				389.42		0.8651115

				389.44		0.8651115

				389.46		0.8651115

				389.48		0.8651115

				389.51		0.8651115

				389.53		0.8651115

				389.55		0.8651115

				389.57		0.8651115

				389.59		0.8651115

				389.61		0.8651115

				389.63		0.8651115

				389.65		0.8651115

				389.68		0.8651115

				389.7		0.8651115

				389.72		0.8651115

				389.74		0.8689916

				389.76		0.8689916

				389.78		0.8689916

				389.8		0.8689916

				389.82		0.8689916

				389.84		0.8689916

				389.87		0.8689916

				389.89		0.8689916

				389.91		0.8689916

				389.93		0.8689916

				389.95		0.8689916

				389.97		0.8689916

				389.99		0.8689916

				390.01		0.8689916

				390.04		0.8689916

				390.06		0.8689916

				390.08		0.8728716

				390.1		0.8728716

				390.12		0.8728716

				390.14		0.8728716

				390.16		0.8728716

				390.18		0.8728716

				390.21		0.8728716

				390.23		0.8728716

				390.25		0.8728716

				390.27		0.8728716

				390.29		0.8728716

				390.31		0.8728716

				390.33		0.8728716

				390.35		0.8728716

				390.38		0.8728716

				390.4		0.8728716

				390.42		0.8728716

				390.44		0.8728716

				390.46		0.8767516

				390.48		0.8728716

				390.5		0.8728716

				390.52		0.8728716

				390.54		0.8728716

				390.57		0.8728716

				390.59		0.8728716

				390.61		0.8728716

				390.63		0.8728716

				390.65		0.8728716

				390.67		0.8728716

				390.69		0.8728716

				390.71		0.8728716

				390.74		0.8728716

				390.76		0.8728716

				390.78		0.8728716

				390.8		0.8728716

				390.82		0.8728716

				390.84		0.8728716

				390.86		0.8728716

				390.88		0.8728716

				390.91		0.8767516

				390.93		0.8767516

				390.95		0.8728716

				390.97		0.8767516

				390.99		0.8767516

				391.01		0.8767516

				391.03		0.8728716

				391.05		0.8767516

				391.08		0.8728716

				391.1		0.8728716

				391.12		0.8728716

				391.14		0.8728716

				391.16		0.8728716

				391.18		0.8728716

				391.2		0.8728716

				391.22		0.8728716

				391.24		0.8728716

				391.27		0.8728716

				391.29		0.8728716

				391.31		0.8728716

				391.33		0.8728716

				391.35		0.8728716

				391.37		0.8728716

				391.39		0.8767516

				391.41		0.8728716

				391.44		0.8728716

				391.46		0.8728716

				391.48		0.8728716

				391.5		0.8728716

				391.52		0.8728716

				391.54		0.8728716

				391.56		0.8767516

				391.58		0.8728716

				391.6		0.8728716

				391.63		0.8728716

				391.65		0.8728716

				391.67		0.8728716

				391.69		0.8728716

		Results:

		Onset		X1		201.93		°C

				Y1		92.988		%

				X2		259.47		°C

				Y2		5.869		%

				Onset X		240.1		°C

				Onset Y		73.522		%
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		Method Filename:		C:\Program Files (x86)\PerkinElmer\Pyris\data\Anas\21052024\RT54.t6d

		Sample ID:		RT54

		Step:		1

		Data		Sample Temperature (°C)		Weight % (%)

				30.11		100.0058

				30.1		100.0058

				30.1		100.0058

				30.1		100.0115

				30.1		100.0115

				30.1		100.0115

				30.1		100.0115

				30.1		100.0115

				30.1		100.0115

				30.1		100.0115

				30.1		100.0115

				30.1		100.0115

				30.1		100.0115

				30.1		100.0173

				30.1		100.0173

				30.1		100.0173

				30.1		100.0173

				30.1		100.0173

				30.1		100.0173

				30.1		100.0231

				30.1		100.0231

				30.1		100.0231

				30.1		100.0231

				30.1		100.0231

				30.1		100.0231

				30.1		100.0289

				30.1		100.0231

				30.1		100.0289

				30.1		100.0289

				30.1		100.0289

				30.1		100.0289

				30.1		100.0289

				30.1		100.0289

				30.1		100.0289

				30.1		100.0289

				30.1		100.0346

				30.1		100.0346

				30.1		100.0346

				30.1		100.0346

				30.1		100.0346

				30.1		100.0404

				30.1		100.0404

				30.1		100.0404

				30.1		100.0404

				30.1		100.0404

				30.1		100.0462

				30.1		100.0462

				30.1		100.0462

				30.1		100.0462

				30.1		100.0519

				30.1		100.0519

				30.1		100.0519

				30.1		100.0519

				30.1		100.0577

				30.1		100.0577

				30.1		100.0577

				30.1		100.0577

				30.1		100.0635

				30.1		100.0635

				30.1		100.0635

				30.1		100.0635

				30.1		100.0635

				30.1		100.0635

				30.1		100.0635

				30.1		100.0635

				30.1		100.0635

				30.1		100.0635

				30.1		100.0693

				30.1		100.0693

				30.1		100.0693

				30.1		100.0693

				30.1		100.0693

				30.1		100.0693

				30.1		100.0693

				30.1		100.075

				30.1		100.075

				30.1		100.075

				30.1		100.075

				30.1		100.075

				30.1		100.075

				30.1		100.075

				30.1		100.075

				30.1		100.075

				30.1		100.075

				30.1		100.075

				30.1		100.075

				30.1		100.075

				30.1		100.0808

				30.1		100.0808

				30.1		100.0808

				30.1		100.0808

				30.1		100.0808

				30.1		100.0808

				30.1		100.0808

				30.1		100.0808

				30.1		100.0866

				30.1		100.0866

				30.1		100.0866

				30.1		100.0866

				30.1		100.0866

				30.1		100.0866

				30.1		100.0866

				30.1		100.0866

				30.1		100.0923

				30.1		100.0923

				30.1		100.0923

				30.1		100.0923

				30.1		100.0923

				30.1		100.0923

				30.1		100.0923

				30.1		100.0923

				30.1		100.0923

				30.1		100.0923

				30.1		100.0981

				30.1		100.0981

				30.1		100.0981

				30.11		100.0981

				30.11		100.0981

				30.11		100.0981

				30.11		100.0981

				30.11		100.1039

				30.11		100.1039

				30.11		100.1039

				30.11		100.1039

				30.11		100.1039

				30.11		100.1039

				30.11		100.1039

				30.11		100.1039

				30.12		100.1039

				30.12		100.1039

				30.12		100.1097

				30.12		100.1097

				30.12		100.1097

				30.12		100.1097

				30.12		100.1097

				30.12		100.1097

				30.13		100.1097

				30.13		100.1154

				30.13		100.1154

				30.13		100.1154

				30.13		100.1154

				30.13		100.1154

				30.13		100.1154

				30.14		100.1154

				30.14		100.1154

				30.14		100.1154

				30.14		100.1154

				30.14		100.1212

				30.15		100.1212

				30.15		100.1212

				30.15		100.1212

				30.15		100.1212

				30.15		100.1212

				30.16		100.1212

				30.16		100.1212

				30.16		100.1212

				30.16		100.1212

				30.16		100.1212

				30.17		100.1212

				30.17		100.1212

				30.17		100.127

				30.17		100.127

				30.18		100.127

				30.18		100.127

				30.18		100.127

				30.18		100.127

				30.19		100.127

				30.19		100.127

				30.19		100.127

				30.2		100.127

				30.2		100.127

				30.2		100.127

				30.2		100.127

				30.21		100.127

				30.21		100.127

				30.21		100.1327

				30.22		100.1327

				30.22		100.1327

				30.22		100.1327

				30.23		100.1327

				30.23		100.1327

				30.23		100.1327

				30.24		100.1327

				30.24		100.1327

				30.24		100.1327

				30.25		100.1327

				30.25		100.1327

				30.25		100.1327

				30.26		100.1327

				30.26		100.1385

				30.26		100.1385

				30.27		100.1385

				30.27		100.1385

				30.28		100.1385

				30.28		100.1385

				30.28		100.1385

				30.29		100.1385

				30.29		100.1385

				30.3		100.1385

				30.3		100.1385

				30.3		100.1385

				30.31		100.1385

				30.31		100.1385

				30.32		100.1385

				30.32		100.1443

				30.33		100.1443

				30.33		100.1443

				30.33		100.1443

				30.34		100.1443

				30.34		100.1443

				30.35		100.1443

				30.35		100.1443

				30.36		100.1443

				30.36		100.1443

				30.37		100.1443

				30.37		100.1443

				30.38		100.1443

				30.38		100.1443

				30.38		100.1443

				30.39		100.1501

				30.39		100.1501

				30.4		100.1501

				30.4		100.1501

				30.41		100.1501

				30.41		100.1501

				30.42		100.1501

				30.42		100.1501

				30.43		100.1501

				30.43		100.1501

				30.44		100.1501

				30.45		100.1558

				30.45		100.1558

				30.46		100.1558

				30.46		100.1558

				30.47		100.1558

				30.47		100.1558

				30.48		100.1558

				30.48		100.1558

				30.49		100.1558

				30.49		100.1558

				30.5		100.1558

				30.51		100.1616

				30.51		100.1616

				30.52		100.1616

				30.52		100.1616

				30.53		100.1616

				30.53		100.1616

				30.54		100.1616

				30.55		100.1616

				30.55		100.1616

				30.56		100.1616

				30.56		100.1616

				30.57		100.1616

				30.58		100.1674

				30.58		100.1674

				30.59		100.1674

				30.59		100.1674

				30.6		100.1674

				30.61		100.1674

				30.61		100.1731

				30.62		100.1731

				30.63		100.1731

				30.63		100.1731

				30.64		100.1731

				30.65		100.1731

				30.65		100.1731

				30.66		100.1731

				30.66		100.1731

				30.67		100.1731

				30.68		100.1731

				30.68		100.1731

				30.69		100.1789

				30.7		100.1731

				30.7		100.1789

				30.71		100.1789

				30.72		100.1789

				30.72		100.1789

				30.73		100.1789

				30.74		100.1789

				30.75		100.1789

				30.75		100.1789

				30.76		100.1789

				30.77		100.1789

				30.77		100.1789

				30.78		100.1789

				30.79		100.1789

				30.79		100.1789

				30.8		100.1847

				30.81		100.1789

				30.82		100.1847

				30.82		100.1847

				30.83		100.1847

				30.84		100.1847

				30.84		100.1847

				30.85		100.1847

				30.86		100.1847

				30.87		100.1847

				30.87		100.1847

				30.88		100.1847

				30.89		100.1847

				30.9		100.1905

				30.9		100.1905

				30.91		100.1905

				30.92		100.1905

				30.93		100.1905

				30.93		100.1905

				30.94		100.1905

				30.95		100.1905

				30.96		100.1905

				30.96		100.1905

				30.97		100.1905

				30.98		100.1905

				30.99		100.1905

				31		100.1905

				31		100.1905

				31.01		100.1905

				31.02		100.1905

				31.03		100.1905

				31.04		100.1905

				31.04		100.1962

				31.05		100.1962

				31.06		100.1962

				31.07		100.1962

				31.08		100.1962

				31.08		100.1962

				31.09		100.1962

				31.1		100.1962

				31.11		100.1962

				31.12		100.1962

				31.12		100.1962

				31.13		100.1905

				31.14		100.1962

				31.15		100.1962

				31.16		100.1962

				31.17		100.1962

				31.17		100.1962

				31.18		100.1962

				31.19		100.1962

				31.2		100.1962

				31.21		100.1962

				31.22		100.1962

				31.22		100.1962

				31.23		100.1962

				31.24		100.1962

				31.25		100.1962

				31.26		100.1962

				31.27		100.202

				31.28		100.202

				31.28		100.202

				31.29		100.1962

				31.3		100.202

				31.31		100.202

				31.32		100.202

				31.33		100.202

				31.34		100.202

				31.35		100.202

				31.35		100.202

				31.36		100.202

				31.37		100.202

				31.38		100.202

				31.39		100.202

				31.4		100.202

				31.41		100.202

				31.42		100.202

				31.43		100.202

				31.44		100.202

				31.44		100.202

				31.45		100.202

				31.46		100.202

				31.47		100.2078

				31.48		100.2078

				31.49		100.2078

				31.5		100.2078

				31.51		100.2078

				31.52		100.2078

				31.53		100.2078

				31.54		100.2078

				31.55		100.2078

				31.55		100.2078

				31.56		100.2078

				31.57		100.2078

				31.58		100.2078

				31.59		100.2078

				31.6		100.2078

				31.61		100.2135

				31.62		100.2078

				31.63		100.2135

				31.64		100.2135

				31.65		100.2135

				31.66		100.2135

				31.67		100.2135

				31.68		100.2135

				31.69		100.2135

				31.7		100.2135

				31.71		100.2135

				31.72		100.2135

				31.73		100.2135

				31.74		100.2135

				31.75		100.2135

				31.76		100.2135

				31.77		100.2135

				31.78		100.2193

				31.79		100.2135

				31.8		100.2135

				31.81		100.2193

				31.82		100.2193

				31.83		100.2193

				31.84		100.2193

				31.85		100.2193

				31.86		100.2193

				31.87		100.2193

				31.88		100.2193

				31.89		100.2193

				31.9		100.2193

				31.91		100.2251

				31.92		100.2193

				31.93		100.2251

				31.94		100.2251

				31.95		100.2251

				31.96		100.2251

				31.97		100.2251

				31.98		100.2251

				31.99		100.2251

				32		100.2251

				32.01		100.2251

				32.02		100.2251

				32.03		100.2309

				32.04		100.2309

				32.05		100.2309

				32.06		100.2309

				32.07		100.2309

				32.08		100.2309

				32.09		100.2309

				32.1		100.2309

				32.11		100.2309

				32.12		100.2309

				32.13		100.2309

				32.14		100.2366

				32.15		100.2366

				32.16		100.2366

				32.18		100.2366

				32.19		100.2366

				32.2		100.2366

				32.21		100.2366

				32.22		100.2366

				32.23		100.2366

				32.24		100.2366

				32.25		100.2366

				32.26		100.2366

				32.27		100.2366

				32.28		100.2366

				32.29		100.2424

				32.3		100.2424

				32.32		100.2424

				32.33		100.2424

				32.34		100.2424

				32.35		100.2424

				32.36		100.2482

				32.37		100.2482

				32.38		100.2482

				32.39		100.2482

				32.4		100.2482

				32.41		100.2482

				32.43		100.2482

				32.44		100.2482

				32.45		100.2539

				32.46		100.2539

				32.47		100.2539

				32.48		100.2539

				32.49		100.2539

				32.5		100.2539

				32.51		100.2539

				32.53		100.2597

				32.54		100.2597

				32.55		100.2597

				32.56		100.2597

				32.57		100.2597

				32.58		100.2597

				32.59		100.2597

				32.61		100.2597

				32.62		100.2597

				32.63		100.2597

				32.64		100.2597

				32.65		100.2597

				32.66		100.2597

				32.67		100.2597

				32.69		100.2597

				32.7		100.2597

				32.71		100.2655

				32.72		100.2597

				32.73		100.2655

				32.74		100.2655

				32.75		100.2655

				32.77		100.2655

				32.78		100.2655

				32.79		100.2655

				32.8		100.2655

				32.81		100.2655

				32.82		100.2655

				32.84		100.2655

				32.85		100.2655

				32.86		100.2713

				32.87		100.2713

				32.88		100.2713

				32.9		100.2713

				32.91		100.2713

				32.92		100.2713

				32.93		100.2713

				32.94		100.2713

				32.96		100.2713

				32.97		100.2713

				32.98		100.2713

				32.99		100.2713

				33		100.2713

				33.01		100.277

				33.03		100.2713

				33.04		100.277

				33.05		100.2713

				33.06		100.277

				33.08		100.277

				33.09		100.277

				33.1		100.277

				33.11		100.277

				33.12		100.277

				33.14		100.277

				33.15		100.277

				33.16		100.277

				33.17		100.277

				33.19		100.277

				33.2		100.277

				33.21		100.277

				33.22		100.277

				33.23		100.277

				33.25		100.277

				33.26		100.277

				33.27		100.277

				33.28		100.277

				33.3		100.277

				33.31		100.277

				33.32		100.277

				33.33		100.277

				33.35		100.277

				33.36		100.277

				33.37		100.277

				33.38		100.277

				33.4		100.277

				33.41		100.2828

				33.42		100.277

				33.43		100.277

				33.45		100.277

				33.46		100.277

				33.47		100.277

				33.48		100.2828

				33.5		100.277

				33.51		100.2828

				33.52		100.277

				33.54		100.2828

				33.55		100.277

				33.56		100.277

				33.57		100.277

				33.59		100.277

				33.6		100.2828

				33.61		100.277

				33.62		100.277

				33.64		100.277

				33.65		100.277

				33.66		100.277

				33.68		100.277

				33.69		100.277

				33.7		100.277

				33.72		100.277

				33.73		100.277

				33.74		100.2828

				33.75		100.2828

				33.77		100.2828

				33.78		100.2828

				33.79		100.2828

				33.81		100.2828

				33.82		100.2828

				33.83		100.2828

				33.85		100.2828

				33.86		100.2828

				33.87		100.2828

				33.89		100.2828

				33.9		100.2828

				33.91		100.2828

				33.93		100.2828

				33.94		100.2828

				33.95		100.2828

				33.96		100.2828

				33.98		100.2828

				33.99		100.2828

				34		100.2828

				34.02		100.2886

				34.03		100.2886

				34.04		100.2886

				34.06		100.2886

				34.07		100.2886

				34.08		100.2886

				34.1		100.2886

				34.11		100.2886

				34.12		100.2886

				34.14		100.2886

				34.15		100.2886

				34.17		100.2886

				34.18		100.2886

				34.19		100.2886

				34.21		100.2886

				34.22		100.2886

				34.23		100.2886

				34.25		100.2886

				34.26		100.2886

				34.27		100.2886

				34.29		100.2886

				34.3		100.2886

				34.31		100.2886

				34.33		100.2886

				34.34		100.2886

				34.36		100.2886

				34.37		100.2886

				34.38		100.2943

				34.4		100.2886

				34.41		100.2943

				34.42		100.2943

				34.44		100.2943

				34.45		100.2943

				34.47		100.2943

				34.48		100.2943

				34.49		100.2943

				34.51		100.2943

				34.52		100.2943

				34.53		100.2943

				34.55		100.2943

				34.56		100.2943

				34.58		100.2943

				34.59		100.2943

				34.6		100.2943

				34.62		100.2943

				34.63		100.2943

				34.65		100.2943

				34.66		100.2943

				34.67		100.2943

				34.69		100.2943

				34.7		100.2943

				34.72		100.2943

				34.73		100.2943

				34.74		100.2943

				34.76		100.3001

				34.77		100.2943

				34.79		100.2943

				34.8		100.2943

				34.82		100.2943

				34.83		100.2943

				34.84		100.2943

				34.86		100.3001

				34.87		100.2943

				34.89		100.2943

				34.9		100.2943

				34.91		100.3001

				34.93		100.2943

				34.94		100.2943

				34.96		100.3001

				34.97		100.3001

				34.99		100.3001

				35		100.3001

				35.02		100.3001

				35.03		100.3001

				35.04		100.3001

				35.06		100.3001

				35.07		100.3001

				35.09		100.3001

				35.1		100.3001

				35.12		100.3001

				35.13		100.3001

				35.14		100.3001

				35.16		100.3001

				35.17		100.3001

				35.19		100.3001

				35.2		100.3001

				35.22		100.2943

				35.23		100.3001

				35.25		100.3001

				35.26		100.3001

				35.28		100.2943

				35.29		100.3001

				35.3		100.2943

				35.32		100.2943

				35.33		100.3001

				35.35		100.2943

				35.36		100.2943

				35.38		100.2943

				35.39		100.3001

				35.41		100.2943

				35.42		100.2943

				35.44		100.2943

				35.45		100.2943

				35.47		100.2943

				35.48		100.2943

				35.5		100.2943

				35.51		100.2943

				35.53		100.2943

				35.54		100.3001

				35.55		100.3001

				35.57		100.3001

				35.58		100.3001

				35.6		100.3001

				35.61		100.3001

				35.63		100.3001

				35.64		100.3001

				35.66		100.3001

				35.67		100.3001

				35.69		100.3001

				35.7		100.3001

				35.72		100.3001

				35.73		100.3001

				35.75		100.3001

				35.76		100.3001

				35.78		100.3001

				35.79		100.3001

				35.81		100.3001

				35.82		100.3001

				35.84		100.3001

				35.85		100.3001

				35.87		100.3001

				35.88		100.3001

				35.9		100.3001

				35.91		100.3001

				35.93		100.3001

				35.94		100.3001

				35.96		100.3001

				35.97		100.3001

				35.99		100.3001

				36		100.3059

				36.02		100.3059

				36.03		100.3059

				36.05		100.3059

				36.06		100.3059

				36.08		100.3059

				36.1		100.3059

				36.11		100.3059

				36.13		100.3001

				36.14		100.3059

				36.16		100.3059

				36.17		100.3059

				36.19		100.3059

				36.2		100.3059

				36.22		100.3059

				36.23		100.3059

				36.25		100.3059

				36.26		100.3059

				36.28		100.3059

				36.29		100.3059

				36.31		100.3059

				36.33		100.3059

				36.34		100.3059

				36.36		100.3059

				36.37		100.3059

				36.39		100.3059

				36.4		100.3059

				36.42		100.3059

				36.43		100.3059

				36.45		100.3059

				36.46		100.3059

				36.48		100.3059

				36.5		100.3117

				36.51		100.3059

				36.53		100.3117

				36.54		100.3117

				36.56		100.3117

				36.57		100.3117

				36.59		100.3117

				36.6		100.3117

				36.62		100.3117

				36.64		100.3117

				36.65		100.3117

				36.67		100.3117

				36.68		100.3117

				36.7		100.3117

				36.71		100.3174

				36.73		100.3174

				36.74		100.3174

				36.76		100.3174

				36.78		100.3174

				36.79		100.3174

				36.81		100.3174

				36.82		100.3174

				36.84		100.3174

				36.85		100.3174

				36.87		100.3174

				36.89		100.3174

				36.9		100.3174

				36.92		100.3174

				36.93		100.3174

				36.95		100.3174

				36.97		100.3174

				36.98		100.3232

				37		100.3232

				37.01		100.3232

				37.03		100.3232

				37.04		100.3232

				37.06		100.3232

				37.08		100.3232

				37.09		100.3232

				37.11		100.3232

				37.12		100.3232

				37.14		100.3232

				37.16		100.3232

				37.17		100.3232

				37.19		100.3232

				37.2		100.3232

				37.22		100.3232

				37.24		100.3232

				37.25		100.3232

				37.27		100.3232

				37.28		100.3232

				37.3		100.3232

				37.32		100.3232

				37.33		100.3232

				37.35		100.3232

				37.36		100.3232

				37.38		100.3232

				37.4		100.3232

				37.41		100.3232

				37.43		100.3232

				37.44		100.3232

				37.46		100.3232

				37.48		100.3232

				37.49		100.3232

				37.51		100.3232

				37.53		100.329

				37.54		100.329

				37.56		100.329

				37.57		100.329

				37.59		100.329

				37.61		100.329

				37.62		100.329

				37.64		100.329

				37.66		100.329

				37.67		100.329

				37.69		100.329

				37.7		100.329

				37.72		100.329

				37.74		100.329

				37.75		100.329

				37.77		100.329

				37.79		100.329

				37.8		100.329

				37.82		100.3347

				37.83		100.3347

				37.85		100.3347

				37.87		100.3347

				37.88		100.3347

				37.9		100.3347

				37.92		100.3347

				37.93		100.3347

				37.95		100.3347

				37.97		100.3347

				37.98		100.3347

				38		100.3347

				38.02		100.3347

				38.03		100.3347

				38.05		100.3347

				38.06		100.3347

				38.08		100.3347

				38.1		100.3347

				38.11		100.3347

				38.13		100.3405

				38.15		100.3347

				38.16		100.3405

				38.18		100.3347

				38.2		100.3347

				38.21		100.3347

				38.23		100.3347

				38.25		100.3405

				38.26		100.3347

				38.28		100.3347

				38.3		100.3405

				38.31		100.3347

				38.33		100.3347

				38.35		100.3347

				38.36		100.3347

				38.38		100.3347

				38.4		100.3347

				38.41		100.3347

				38.43		100.3347

				38.45		100.3347

				38.46		100.3347

				38.48		100.3347

				38.5		100.3347

				38.51		100.3347

				38.53		100.3347

				38.55		100.3347

				38.56		100.3347

				38.58		100.3347

				38.6		100.3347

				38.61		100.3347

				38.63		100.3347

				38.65		100.3405

				38.66		100.3405

				38.68		100.3405

				38.7		100.3405

				38.71		100.3405

				38.73		100.3405

				38.75		100.3405

				38.76		100.3405

				38.78		100.3405

				38.8		100.3405

				38.82		100.3405

				38.83		100.3405

				38.85		100.3405

				38.87		100.3405

				38.88		100.3405

				38.9		100.3405

				38.92		100.3405

				38.93		100.3405

				38.95		100.3405

				38.97		100.3405

				38.98		100.3405

				39		100.3405

				39.02		100.3405

				39.04		100.3405

				39.05		100.3405

				39.07		100.3405

				39.09		100.3405

				39.1		100.3463

				39.12		100.3405

				39.14		100.3405

				39.15		100.3405

				39.17		100.3405

				39.19		100.3405

				39.21		100.3405

				39.22		100.3463

				39.24		100.3405

				39.26		100.3463

				39.27		100.3463

				39.29		100.3463

				39.31		100.3463

				39.33		100.3463

				39.34		100.3463

				39.36		100.3463

				39.38		100.3463

				39.39		100.3463

				39.41		100.3463

				39.43		100.3463

				39.45		100.3463

				39.46		100.3463

				39.48		100.3463

				39.5		100.3463

				39.51		100.3463

				39.53		100.3463

				39.55		100.3463

				39.57		100.3463

				39.58		100.3521

				39.6		100.3521

				39.62		100.3521

				39.63		100.3521

				39.65		100.3521

				39.67		100.3521

				39.69		100.3521

				39.7		100.3521

				39.72		100.3521

				39.74		100.3521

				39.76		100.3521

				39.77		100.3521

				39.79		100.3521

				39.81		100.3521

				39.83		100.3521

				39.84		100.3521

				39.86		100.3521

				39.88		100.3521

				39.89		100.3521

				39.91		100.3521

				39.93		100.3521

				39.95		100.3521

				39.96		100.3521

				39.98		100.3521

				40		100.3521

				40.02		100.3521

				40.03		100.3521

				40.05		100.3578

				40.07		100.3578

				40.09		100.3578

				40.1		100.3578

				40.12		100.3578

				40.14		100.3578

				40.16		100.3578

				40.17		100.3578

				40.19		100.3578

				40.21		100.3578

				40.23		100.3578

				40.24		100.3578

				40.26		100.3578

				40.28		100.3578

				40.3		100.3636

				40.31		100.3578

				40.33		100.3578

				40.35		100.3578

				40.37		100.3578

				40.38		100.3578

				40.4		100.3578

				40.42		100.3578

				40.44		100.3578

				40.45		100.3578

				40.47		100.3578

				40.49		100.3636

				40.51		100.3636

				40.52		100.3578

				40.54		100.3636

				40.56		100.3636

				40.58		100.3636

				40.59		100.3636

				40.61		100.3636

				40.63		100.3636

				40.65		100.3636

				40.67		100.3636

				40.68		100.3636

				40.7		100.3636

				40.72		100.3636

				40.74		100.3636

				40.75		100.3636

				40.77		100.3636

				40.79		100.3636

				40.81		100.3636

				40.82		100.3636

				40.84		100.3636

				40.86		100.3636

				40.88		100.3636

				40.9		100.3636

				40.91		100.3636

				40.93		100.3636

				40.95		100.3636

				40.97		100.3636

				40.98		100.3694

				41		100.3694

				41.02		100.3636

				41.04		100.3636

				41.06		100.3694

				41.07		100.3636

				41.09		100.3636

				41.11		100.3636

				41.13		100.3636

				41.15		100.3636

				41.16		100.3636

				41.18		100.3636

				41.2		100.3636

				41.22		100.3636

				41.23		100.3636

				41.25		100.3636

				41.27		100.3636

				41.29		100.3694

				41.31		100.3694

				41.32		100.3636

				41.34		100.3694

				41.36		100.3694

				41.38		100.3694

				41.4		100.3694

				41.41		100.3694

				41.43		100.3694

				41.45		100.3694

				41.47		100.3694

				41.49		100.3694

				41.5		100.3694

				41.52		100.3751

				41.54		100.3751

				41.56		100.3694

				41.58		100.3751

				41.59		100.3751

				41.61		100.3751

				41.63		100.3751

				41.65		100.3751

				41.67		100.3751

				41.68		100.3751

				41.7		100.3751

				41.72		100.3751

				41.74		100.3751

				41.76		100.3751

				41.77		100.3751

				41.79		100.3751

				41.81		100.3751

				41.83		100.3751

				41.85		100.3751

				41.86		100.3751

				41.88		100.3751

				41.9		100.3751

				41.92		100.3751

				41.94		100.3751

				41.96		100.3751

				41.97		100.3751

				41.99		100.3751

				42.01		100.3751

				42.03		100.3751

				42.05		100.3751

				42.06		100.3751

				42.08		100.3809

				42.1		100.3809

				42.12		100.3809

				42.14		100.3809

				42.15		100.3809

				42.17		100.3809

				42.19		100.3809

				42.21		100.3809

				42.23		100.3809

				42.25		100.3809

				42.26		100.3809

				42.28		100.3809

				42.3		100.3809

				42.32		100.3809

				42.34		100.3809

				42.36		100.3809

				42.37		100.3809

				42.39		100.3809

				42.41		100.3809

				42.43		100.3809

				42.45		100.3809

				42.47		100.3809

				42.48		100.3809

				42.5		100.3867

				42.52		100.3809

				42.54		100.3809

				42.56		100.3809

				42.57		100.3867

				42.59		100.3867

				42.61		100.3867

				42.63		100.3867

				42.65		100.3867

				42.67		100.3867

				42.68		100.3867

				42.7		100.3867

				42.72		100.3867

				42.74		100.3867

				42.76		100.3867

				42.78		100.3867

				42.8		100.3867

				42.81		100.3867

				42.83		100.3867

				42.85		100.3867

				42.87		100.3867

				42.89		100.3867

				42.91		100.3867

				42.92		100.3867

				42.94		100.3867

				42.96		100.3925

				42.98		100.3867

				43		100.3925

				43.02		100.3867

				43.03		100.3925

				43.05		100.3925

				43.07		100.3925

				43.09		100.3867

				43.11		100.3867

				43.13		100.3867

				43.15		100.3867

				43.16		100.3867

				43.18		100.3867

				43.2		100.3867

				43.22		100.3867

				43.24		100.3867

				43.26		100.3867

				43.28		100.3867

				43.29		100.3867

				43.31		100.3867

				43.33		100.3867

				43.35		100.3867

				43.37		100.3867

				43.39		100.3867

				43.4		100.3867

				43.42		100.3867

				43.44		100.3867

				43.46		100.3867

				43.48		100.3867

				43.5		100.3867

				43.52		100.3867

				43.53		100.3867

				43.55		100.3867

				43.57		100.3867

				43.59		100.3867

				43.61		100.3867

				43.63		100.3867

				43.65		100.3867

				43.67		100.3867

				43.68		100.3867

				43.7		100.3867

				43.72		100.3867

				43.74		100.3867

				43.76		100.3867

				43.78		100.3867

				43.8		100.3867

				43.81		100.3867

				43.83		100.3867

				43.85		100.3867

				43.87		100.3867

				43.89		100.3867

				43.91		100.3867

				43.93		100.3867

				43.95		100.3867

				43.96		100.3867

				43.98		100.3867

				44		100.3867

				44.02		100.3867

				44.04		100.3867

				44.06		100.3867

				44.08		100.3867

				44.1		100.3867

				44.11		100.3867

				44.13		100.3867

				44.15		100.3867

				44.17		100.3867

				44.19		100.3867

				44.21		100.3867

				44.23		100.3867

				44.25		100.3867

				44.26		100.3867

				44.28		100.3867

				44.3		100.3925

				44.32		100.3867

				44.34		100.3925

				44.36		100.3925

				44.38		100.3925

				44.4		100.3925

				44.41		100.3925

				44.43		100.3925

				44.45		100.3925

				44.47		100.3925

				44.49		100.3925

				44.51		100.3867

				44.53		100.3925

				44.55		100.3925

				44.57		100.3925

				44.58		100.3925

				44.6		100.3925

				44.62		100.3925

				44.64		100.3925

				44.66		100.3925

				44.68		100.3925

				44.7		100.3925

				44.72		100.3925

				44.74		100.3925

				44.75		100.3925

				44.77		100.3925

				44.79		100.3982

				44.81		100.3982

				44.83		100.3982

				44.85		100.3982

				44.87		100.3982

				44.89		100.3982

				44.91		100.3982

				44.92		100.3982

				44.94		100.3982

				44.96		100.3982

				44.98		100.3982

				45		100.3982

				45.02		100.3982

				45.04		100.3982

				45.06		100.404

				45.08		100.404

				45.1		100.404

				45.11		100.404

				45.13		100.404

				45.15		100.404

				45.17		100.404

				45.19		100.404

				45.21		100.404

				45.23		100.404

				45.25		100.404

				45.27		100.4098

				45.29		100.4098

				45.3		100.4098

				45.32		100.4098

				45.34		100.4098

				45.36		100.4098

				45.38		100.4098

				45.4		100.4098

				45.42		100.4098

				45.44		100.4098

				45.46		100.4098

				45.48		100.4098

				45.49		100.4155

				45.51		100.4155

				45.53		100.4155

				45.55		100.4155

				45.57		100.4155

				45.59		100.4155

				45.61		100.4155

				45.63		100.4155

				45.65		100.4155

				45.67		100.4213

				45.69		100.4213

				45.7		100.4213

				45.72		100.4213

				45.74		100.4213

				45.76		100.4213

				45.78		100.4213

				45.8		100.4271

				45.82		100.4271

				45.84		100.4271

				45.86		100.4271

				45.88		100.4271

				45.9		100.4271

				45.91		100.4271

				45.93		100.4271

				45.95		100.4271

				45.97		100.4271

				45.99		100.4271

				46.01		100.4271

				46.03		100.4329

				46.05		100.4329

				46.07		100.4329

				46.09		100.4329

				46.11		100.4329

				46.13		100.4329

				46.14		100.4329

				46.16		100.4329

				46.18		100.4329

				46.2		100.4329

				46.22		100.4329

				46.24		100.4329

				46.26		100.4329

				46.28		100.4329

				46.3		100.4329

				46.32		100.4329

				46.34		100.4329

				46.36		100.4386

				46.38		100.4386

				46.39		100.4386

				46.41		100.4386

				46.43		100.4386

				46.45		100.4386

				46.47		100.4386

				46.49		100.4386

				46.51		100.4386

				46.53		100.4386

				46.55		100.4386

				46.57		100.4386

				46.59		100.4386

				46.61		100.4386

				46.63		100.4386

				46.65		100.4386

				46.66		100.4386

				46.68		100.4386

				46.7		100.4386

				46.72		100.4386

				46.74		100.4386

				46.76		100.4386

				46.78		100.4386

				46.8		100.4386

				46.82		100.4386

				46.84		100.4386

				46.86		100.4386

				46.88		100.4444

				46.9		100.4386

				46.92		100.4386

				46.94		100.4386

				46.95		100.4386

				46.97		100.4386

				46.99		100.4386

				47.01		100.4386

				47.03		100.4386

				47.05		100.4386

				47.07		100.4386

				47.09		100.4386

				47.11		100.4386

				47.13		100.4386

				47.15		100.4386

				47.17		100.4386

				47.19		100.4386

				47.21		100.4444

				47.23		100.4386

				47.25		100.4386

				47.26		100.4444

				47.28		100.4444

				47.3		100.4444

				47.32		100.4444

				47.34		100.4444

				47.36		100.4444

				47.38		100.4444

				47.4		100.4444

				47.42		100.4444

				47.44		100.4386

				47.46		100.4386

				47.48		100.4386

				47.5		100.4386

				47.52		100.4386

				47.54		100.4386

				47.56		100.4386

				47.58		100.4386

				47.59		100.4386

				47.61		100.4386

				47.63		100.4386

				47.65		100.4386

				47.67		100.4386

				47.69		100.4386

				47.71		100.4386

				47.73		100.4386

				47.75		100.4386

				47.77		100.4386

				47.79		100.4386

				47.81		100.4386

				47.83		100.4386

				47.85		100.4386

				47.87		100.4386

				47.89		100.4386

				47.91		100.4386

				47.93		100.4386

				47.95		100.4386

				47.97		100.4386

				47.98		100.4386

				48		100.4386

				48.02		100.4386

				48.04		100.4386

				48.06		100.4386

				48.08		100.4386

				48.1		100.4386

				48.12		100.4386

				48.14		100.4386

				48.16		100.4386

				48.18		100.4386

				48.2		100.4386

				48.22		100.4386

				48.24		100.4386

				48.26		100.4386

				48.28		100.4386

				48.3		100.4386

				48.32		100.4386

				48.34		100.4386

				48.36		100.4386

				48.38		100.4386

				48.39		100.4386

				48.41		100.4386

				48.43		100.4386

				48.45		100.4386

				48.47		100.4386

				48.49		100.4386

				48.51		100.4386

				48.53		100.4386

				48.55		100.4386

				48.57		100.4386

				48.59		100.4386

				48.61		100.4386

				48.63		100.4386

				48.65		100.4386

				48.67		100.4386

				48.69		100.4386

				48.71		100.4386

				48.73		100.4386

				48.75		100.4386

				48.77		100.4386

				48.79		100.4386

				48.81		100.4386

				48.83		100.4386

				48.85		100.4386

				48.87		100.4386

				48.89		100.4386

				48.91		100.4386

				48.93		100.4386

				48.94		100.4386

				48.96		100.4386

				48.98		100.4386

				49		100.4386

				49.02		100.4386

				49.04		100.4386

				49.06		100.4386

				49.08		100.4386

				49.1		100.4386

				49.12		100.4386

				49.14		100.4386

				49.16		100.4386

				49.18		100.4386

				49.2		100.4386

				49.22		100.4386

				49.24		100.4386

				49.26		100.4386

				49.28		100.4386

				49.3		100.4386

				49.32		100.4386

				49.34		100.4386

				49.36		100.4386

				49.38		100.4386

				49.4		100.4386

				49.42		100.4386

				49.44		100.4386

				49.46		100.4386

				49.48		100.4386

				49.5		100.4386

				49.52		100.4386

				49.54		100.4386

				49.56		100.4386

				49.58		100.4386

				49.6		100.4386

				49.62		100.4386

				49.64		100.4386

				49.66		100.4386

				49.68		100.4386

				49.7		100.4386

				49.71		100.4386

				49.73		100.4386

				49.75		100.4386

				49.77		100.4386

				49.79		100.4386

				49.81		100.4386

				49.83		100.4386

				49.85		100.4386

				49.87		100.4386

				49.89		100.4386

				49.91		100.4386

				49.93		100.4386

				49.95		100.4386

				49.97		100.4386

				49.99		100.4386

				50.01		100.4386

				50.03		100.4444

				50.05		100.4386

				50.07		100.4386

				50.09		100.4386

				50.11		100.4386

				50.13		100.4386

				50.15		100.4386

				50.17		100.4386

				50.19		100.4386

				50.21		100.4386

				50.23		100.4386

				50.25		100.4444

				50.27		100.4386

				50.29		100.4444

				50.31		100.4444

				50.33		100.4444

				50.35		100.4444

				50.37		100.4444

				50.39		100.4444

				50.41		100.4444

				50.43		100.4444

				50.45		100.4444

				50.47		100.4444

				50.49		100.4444

				50.51		100.4444

				50.53		100.4444

				50.55		100.4444

				50.57		100.4444

				50.59		100.4444

				50.61		100.4444

				50.63		100.4444

				50.65		100.4444

				50.67		100.4444

				50.69		100.4444

				50.71		100.4444

				50.73		100.4444

				50.75		100.4444

				50.77		100.4444

				50.79		100.4502

				50.81		100.4502

				50.83		100.4502

				50.85		100.4502

				50.87		100.4502

				50.89		100.4502

				50.91		100.4502

				50.93		100.4502

				50.95		100.4502

				50.97		100.4502

				50.99		100.4502

				51.01		100.4502

				51.03		100.4502

				51.05		100.4502

				51.07		100.4502

				51.09		100.4502

				51.11		100.4559

				51.13		100.4559

				51.15		100.4559

				51.17		100.4559

				51.19		100.4559

				51.21		100.4559

				51.23		100.4559

				51.25		100.4559

				51.27		100.4559

				51.29		100.4559

				51.31		100.4559

				51.33		100.4559

				51.35		100.4617

				51.37		100.4559

				51.39		100.4617

				51.41		100.4617

				51.43		100.4617

				51.45		100.4617

				51.47		100.4617

				51.49		100.4617

				51.51		100.4617

				51.53		100.4675

				51.55		100.4675

				51.57		100.4675

				51.59		100.4675

				51.61		100.4675

				51.63		100.4675

				51.65		100.4675

				51.67		100.4675

				51.69		100.4675

				51.71		100.4675

				51.73		100.4675

				51.75		100.4675

				51.77		100.4675

				51.79		100.4675

				51.81		100.4675

				51.83		100.4732

				51.85		100.4675

				51.87		100.4732

				51.89		100.4732

				51.91		100.4732

				51.93		100.4732

				51.95		100.4732

				51.97		100.4732

				51.99		100.4675

				52.01		100.4732

				52.03		100.4732

				52.05		100.4732

				52.07		100.4732

				52.09		100.4732

				52.11		100.4732

				52.13		100.4732

				52.15		100.4732

				52.17		100.4732

				52.19		100.4732

				52.21		100.4732

				52.23		100.4732

				52.25		100.4732

				52.27		100.4732

				52.29		100.4732

				52.31		100.4732

				52.33		100.4732

				52.35		100.4732

				52.37		100.4732

				52.39		100.4732

				52.41		100.4732

				52.43		100.4732

				52.45		100.4732

				52.47		100.4732

				52.49		100.4732

				52.51		100.4732

				52.53		100.4732

				52.55		100.4732

				52.57		100.4732

				52.59		100.4732

				52.61		100.4732

				52.63		100.4732

				52.65		100.4732

				52.67		100.4732

				52.69		100.4732

				52.71		100.4732

				52.73		100.4732

				52.75		100.4732

				52.77		100.4732

				52.79		100.4732

				52.81		100.4732

				52.83		100.4732

				52.85		100.4732

				52.87		100.4732

				52.89		100.4732

				52.91		100.4732

				52.93		100.4732

				52.95		100.4732

				52.97		100.4732

				52.99		100.4732

				53.01		100.4732

				53.03		100.4732

				53.05		100.4732

				53.07		100.4732

				53.09		100.4732

				53.11		100.4732

				53.13		100.4732

				53.15		100.4732

				53.17		100.4732

				53.19		100.4732

				53.21		100.4732

				53.23		100.4732

				53.25		100.4732

				53.27		100.4732

				53.3		100.4732

				53.32		100.4732

				53.34		100.4732

				53.36		100.4732

				53.38		100.4675

				53.4		100.4732

				53.42		100.4732

				53.44		100.4732

				53.46		100.4675

				53.48		100.4675

				53.5		100.4675

				53.52		100.4675

				53.54		100.4732

				53.56		100.4675

				53.58		100.4675

				53.6		100.4675

				53.62		100.4732

				53.64		100.4675

				53.66		100.4732

				53.68		100.4732

				53.7		100.4732

				53.72		100.4732

				53.74		100.4732

				53.76		100.4732

				53.78		100.4732

				53.8		100.4732

				53.82		100.4732

				53.84		100.4732

				53.86		100.4732

				53.88		100.4732

				53.9		100.4732

				53.92		100.4732

				53.94		100.4732

				53.96		100.4732

				53.98		100.4732

				54		100.4732

				54.02		100.4732

				54.04		100.4732

				54.06		100.4732

				54.08		100.4732

				54.1		100.4732

				54.12		100.4732

				54.15		100.4732

				54.17		100.4732

				54.19		100.4732

				54.21		100.4732

				54.23		100.479

				54.25		100.479

				54.27		100.479

				54.29		100.4732

				54.31		100.479

				54.33		100.479

				54.35		100.479

				54.37		100.4732

				54.39		100.479

				54.41		100.4732

				54.43		100.4732

				54.45		100.4732

				54.47		100.4732

				54.49		100.4732

				54.51		100.479

				54.53		100.4732

				54.55		100.479

				54.57		100.479

				54.59		100.479

				54.61		100.479

				54.63		100.479

				54.65		100.479

				54.67		100.479

				54.69		100.479

				54.71		100.479

				54.73		100.479

				54.75		100.479

				54.77		100.479

				54.79		100.479

				54.81		100.479

				54.83		100.479

				54.85		100.479

				54.88		100.479

				54.9		100.479

				54.92		100.479

				54.94		100.479

				54.96		100.479

				54.98		100.479

				55		100.479

				55.02		100.479

				55.04		100.479

				55.06		100.479

				55.08		100.479

				55.1		100.479

				55.12		100.479

				55.14		100.479

				55.16		100.479

				55.18		100.479

				55.2		100.479

				55.22		100.479

				55.24		100.479

				55.26		100.479

				55.28		100.479

				55.3		100.479

				55.32		100.479

				55.34		100.479

				55.36		100.479

				55.38		100.479

				55.4		100.479

				55.42		100.479

				55.44		100.479

				55.46		100.479

				55.49		100.479

				55.51		100.479

				55.53		100.479

				55.55		100.479

				55.57		100.479

				55.59		100.479

				55.61		100.479

				55.63		100.479

				55.65		100.479

				55.67		100.479

				55.69		100.479

				55.71		100.479

				55.73		100.479

				55.75		100.479

				55.77		100.479

				55.79		100.479

				55.81		100.4732

				55.83		100.479

				55.85		100.479

				55.87		100.479

				55.89		100.479

				55.91		100.479

				55.93		100.479

				55.95		100.479

				55.97		100.479

				56		100.479

				56.02		100.479

				56.04		100.479

				56.06		100.479

				56.08		100.479

				56.1		100.479

				56.12		100.479

				56.14		100.479

				56.16		100.479

				56.18		100.479

				56.2		100.479

				56.22		100.4732

				56.24		100.4732

				56.26		100.4732

				56.28		100.479

				56.3		100.4732

				56.32		100.479

				56.34		100.479

				56.36		100.479

				56.38		100.479

				56.4		100.479

				56.42		100.479

				56.45		100.479

				56.47		100.479

				56.49		100.479

				56.51		100.479

				56.53		100.479

				56.55		100.479

				56.57		100.479

				56.59		100.479

				56.61		100.479

				56.63		100.479

				56.65		100.4848

				56.67		100.4848

				56.69		100.4848

				56.71		100.4848

				56.73		100.4848

				56.75		100.4848

				56.77		100.479

				56.79		100.4848

				56.81		100.4848

				56.83		100.4848

				56.85		100.4848

				56.87		100.4848

				56.9		100.4848

				56.92		100.4848

				56.94		100.4848

				56.96		100.4848

				56.98		100.4848

				57		100.4848

				57.02		100.4848

				57.04		100.4848

				57.06		100.4848

				57.08		100.4848

				57.1		100.4848

				57.12		100.4848

				57.14		100.4906

				57.16		100.4906

				57.18		100.4906

				57.2		100.4906

				57.22		100.4906

				57.24		100.4906

				57.26		100.4906

				57.28		100.4906

				57.3		100.4906

				57.33		100.4906

				57.35		100.4906

				57.37		100.4906

				57.39		100.4963

				57.41		100.4963

				57.43		100.4963

				57.45		100.4963

				57.47		100.4963

				57.49		100.4963

				57.51		100.4963

				57.53		100.4963

				57.55		100.4963

				57.57		100.4963

				57.59		100.4963

				57.61		100.4963

				57.63		100.4963

				57.65		100.4963

				57.67		100.4963

				57.69		100.4963

				57.72		100.4963

				57.74		100.4963

				57.76		100.4963

				57.78		100.5021

				57.8		100.4963

				57.82		100.5021

				57.84		100.5021

				57.86		100.5021

				57.88		100.5021

				57.9		100.5021

				57.92		100.5021

				57.94		100.5021

				57.96		100.5021

				57.98		100.5021

				58		100.5021

				58.02		100.5021

				58.04		100.5021

				58.06		100.5021

				58.08		100.5021

				58.11		100.5021

				58.13		100.5021

				58.15		100.5021

				58.17		100.5021

				58.19		100.5079

				58.21		100.5079

				58.23		100.5079

				58.25		100.5079

				58.27		100.5079

				58.29		100.5079

				58.31		100.5079

				58.33		100.5079

				58.35		100.5079

				58.37		100.5079

				58.39		100.5079

				58.41		100.5079

				58.43		100.5079

				58.45		100.5079

				58.48		100.5079

				58.5		100.5079

				58.52		100.5079

				58.54		100.5079

				58.56		100.5079

				58.58		100.5079

				58.6		100.5079

				58.62		100.5079

				58.64		100.5079

				58.66		100.5079

				58.68		100.5079

				58.7		100.5079

				58.72		100.5079

				58.74		100.5079

				58.76		100.5079

				58.78		100.5079

				58.8		100.5136

				58.82		100.5079

				58.85		100.5136

				58.87		100.5136

				58.89		100.5079

				58.91		100.5079

				58.93		100.5079

				58.95		100.5136

				58.97		100.5136

				58.99		100.5136

				59.01		100.5136

				59.03		100.5136

				59.05		100.5136

				59.07		100.5136

				59.09		100.5136

				59.11		100.5136

				59.13		100.5136

				59.15		100.5136

				59.17		100.5136

				59.2		100.5136

				59.22		100.5136

				59.24		100.5136

				59.26		100.5136

				59.28		100.5136

				59.3		100.5136

				59.32		100.5136

				59.34		100.5136

				59.36		100.5136

				59.38		100.5136

				59.4		100.5136

				59.42		100.5136

				59.44		100.5136

				59.46		100.5136

				59.48		100.5136

				59.5		100.5136

				59.52		100.5136

				59.54		100.5136

				59.57		100.5136

				59.59		100.5136

				59.61		100.5136

				59.63		100.5136

				59.65		100.5136

				59.67		100.5136

				59.69		100.5136

				59.71		100.5194

				59.73		100.5136

				59.75		100.5136

				59.77		100.5194

				59.79		100.5194

				59.81		100.5194

				59.83		100.5194

				59.85		100.5194

				59.87		100.5194

				59.9		100.5194

				59.92		100.5194

				59.94		100.5194

				59.96		100.5194

				59.98		100.5194

				60		100.5194

				60.02		100.5194

				60.04		100.5194

				60.06		100.5252

				60.08		100.5252

				60.1		100.5252

				60.12		100.5252

				60.14		100.5194

				60.16		100.5252

				60.18		100.5252

				60.2		100.5252

				60.22		100.5252

				60.25		100.5252

				60.27		100.5252

				60.29		100.5252

				60.31		100.5252

				60.33		100.5252

				60.35		100.5252

				60.37		100.5252

				60.39		100.5252

				60.41		100.5252

				60.43		100.5252

				60.45		100.5252

				60.47		100.5252

				60.49		100.5252

				60.51		100.5252

				60.53		100.531

				60.55		100.531

				60.57		100.531

				60.59		100.531

				60.62		100.531

				60.64		100.531

				60.66		100.531

				60.68		100.531

				60.7		100.531

				60.72		100.531

				60.74		100.531

				60.76		100.531

				60.78		100.531

				60.8		100.531

				60.82		100.531

				60.84		100.531

				60.86		100.5367

				60.88		100.5367

				60.9		100.5367

				60.92		100.5367

				60.94		100.5367

				60.96		100.5367

				60.99		100.5367

				61.01		100.5367

				61.03		100.5367

				61.05		100.5367

				61.07		100.5367

				61.09		100.5367

				61.11		100.5367

				61.13		100.5367

				61.15		100.5367

				61.17		100.5367

				61.19		100.5367

				61.21		100.5367

				61.23		100.5367

				61.25		100.5367

				61.27		100.5367

				61.29		100.5367

				61.31		100.5367

				61.33		100.5367

				61.36		100.5367

				61.38		100.5425

				61.4		100.5367

				61.42		100.5367

				61.44		100.5425

				61.46		100.5367

				61.48		100.5367

				61.5		100.5367

				61.52		100.5425

				61.54		100.5425

				61.56		100.5425

				61.58		100.5425

				61.6		100.5425

				61.62		100.5425

				61.64		100.5425

				61.66		100.5425

				61.68		100.5425

				61.7		100.5425

				61.73		100.5425

				61.75		100.5425

				61.77		100.5425

				61.79		100.5425

				61.81		100.5425

				61.83		100.5425

				61.85		100.5425

				61.87		100.5425

				61.89		100.5425

				61.91		100.5425

				61.93		100.5425

				61.95		100.5425

				61.97		100.5425

				61.99		100.5425

				62.01		100.5425

				62.03		100.5425

				62.05		100.5425

				62.07		100.5425

				62.1		100.5425

				62.12		100.5425

				62.14		100.5425

				62.16		100.5425

				62.18		100.5483

				62.2		100.5425

				62.22		100.5425

				62.24		100.5425

				62.26		100.5483

				62.28		100.5483

				62.3		100.5483

				62.32		100.5483

				62.34		100.5483

				62.36		100.5483

				62.38		100.5425

				62.4		100.5483

				62.42		100.5483

				62.44		100.5483

				62.46		100.5483

				62.49		100.5483

				62.51		100.5483

				62.53		100.5483

				62.55		100.5483

				62.57		100.5483

				62.59		100.5483

				62.61		100.5483

				62.63		100.5483

				62.65		100.5483

				62.67		100.5483

				62.69		100.5483

				62.71		100.5483

				62.73		100.5483

				62.75		100.5483

				62.77		100.5483

				62.79		100.5483

				62.81		100.5483

				62.83		100.5483

				62.86		100.5425

				62.88		100.5425

				62.9		100.5483

				62.92		100.5425

				62.94		100.5425

				62.96		100.5425

				62.98		100.5425

				63		100.5425

				63.02		100.5483

				63.04		100.5483

				63.06		100.5483

				63.08		100.5483

				63.1		100.5483

				63.12		100.5483

				63.14		100.5483

				63.16		100.5483

				63.18		100.5483

				63.2		100.5483

				63.23		100.5483

				63.25		100.5483

				63.27		100.5483

				63.29		100.5483

				63.31		100.5483

				63.33		100.5425

				63.35		100.5425

				63.37		100.5425

				63.39		100.5425

				63.41		100.5425

				63.43		100.5425

				63.45		100.5425

				63.47		100.5425

				63.49		100.5425

				63.51		100.5483

				63.53		100.5483

				63.55		100.5483

				63.57		100.5483

				63.6		100.5483

				63.62		100.5483

				63.64		100.5483

				63.66		100.5483

				63.68		100.5483

				63.7		100.5483

				63.72		100.5483

				63.74		100.5483

				63.76		100.5483

				63.78		100.5483

				63.8		100.5483

				63.82		100.5483

				63.84		100.5483

				63.86		100.5483

				63.88		100.5483

				63.9		100.5483

				63.92		100.5483

				63.95		100.5483

				63.97		100.5483

				63.99		100.5483

				64.01		100.5483

				64.03		100.5483

				64.05		100.5483

				64.07		100.5483

				64.09		100.5483

				64.11		100.5483

				64.13		100.5483

				64.15		100.5483

				64.17		100.5483

				64.19		100.5425

				64.21		100.5483

				64.23		100.5483

				64.25		100.5425

				64.27		100.5425

				64.29		100.5425

				64.32		100.5425

				64.34		100.5425

				64.36		100.5483

				64.38		100.5483

				64.4		100.5483

				64.42		100.5483

				64.44		100.5483

				64.46		100.5483

				64.48		100.5483

				64.5		100.5483

				64.52		100.5483

				64.54		100.5483

				64.56		100.5483

				64.58		100.5483

				64.6		100.5425

				64.62		100.5483

				64.64		100.5425

				64.67		100.5425

				64.69		100.5425

				64.71		100.5425

				64.73		100.5425

				64.75		100.5425

				64.77		100.5425

				64.79		100.5425

				64.81		100.5425

				64.83		100.5425

				64.85		100.5425

				64.87		100.5425

				64.89		100.5425

				64.91		100.5425

				64.93		100.5425

				64.95		100.5425

				64.97		100.5425

				65		100.5425

				65.02		100.5425

				65.04		100.5425

				65.06		100.5425

				65.08		100.5425

				65.1		100.5425

				65.12		100.5425

				65.14		100.5425

				65.16		100.5425

				65.18		100.5425

				65.2		100.5425

				65.22		100.5425

				65.24		100.5367

				65.26		100.5425

				65.28		100.5367

				65.3		100.5425

				65.33		100.5425

				65.35		100.5425

				65.37		100.5425

				65.39		100.5425

				65.41		100.5425

				65.43		100.5425

				65.45		100.5425

				65.47		100.5425

				65.49		100.5425

				65.51		100.5425

				65.53		100.5425

				65.55		100.5425

				65.57		100.5425

				65.59		100.5425

				65.61		100.5425

				65.63		100.5425

				65.66		100.5425

				65.68		100.5425

				65.7		100.5367

				65.72		100.5367

				65.74		100.5425

				65.76		100.5425

				65.78		100.5425

				65.8		100.5425

				65.82		100.5425

				65.84		100.5425

				65.86		100.5425

				65.88		100.5425

				65.9		100.5425

				65.92		100.5425

				65.94		100.5425

				65.96		100.5425

				65.99		100.5425

				66.01		100.5425

				66.03		100.5425

				66.05		100.5425

				66.07		100.5425

				66.09		100.5367

				66.11		100.5425

				66.13		100.5367

				66.15		100.5425

				66.17		100.5425

				66.19		100.5425

				66.21		100.5425

				66.23		100.5425

				66.25		100.5425

				66.28		100.5425

				66.3		100.5425

				66.32		100.5425

				66.34		100.5425

				66.36		100.5425

				66.38		100.5425

				66.4		100.5425

				66.42		100.5425

				66.44		100.5425

				66.46		100.5425

				66.48		100.5425

				66.5		100.5425

				66.52		100.5425

				66.54		100.5425

				66.57		100.5367

				66.59		100.5425

				66.61		100.5425

				66.63		100.5425

				66.65		100.5425

				66.67		100.5425

				66.69		100.5425

				66.71		100.5425

				66.73		100.5425

				66.75		100.5425

				66.77		100.5425

				66.79		100.5425

				66.81		100.5425

				66.83		100.5425

				66.86		100.5425

				66.88		100.5425

				66.9		100.5425

				66.92		100.5425

				66.94		100.5425

				66.96		100.5425

				66.98		100.5425

				67		100.5425

				67.02		100.5425

				67.04		100.5425

				67.06		100.5425

				67.08		100.5425

				67.1		100.5425

				67.12		100.5425

				67.15		100.5425

				67.17		100.5425

				67.19		100.5425

				67.21		100.5425

				67.23		100.5425

				67.25		100.5425

				67.27		100.5425

				67.29		100.5483

				67.31		100.5425

				67.33		100.5425

				67.35		100.5425

				67.37		100.5483

				67.39		100.5425

				67.41		100.5425

				67.44		100.5425

				67.46		100.5425

				67.48		100.5425

				67.5		100.5425

				67.52		100.5425

				67.54		100.5425

				67.56		100.5425

				67.58		100.5425

				67.6		100.5425

				67.62		100.5425

				67.64		100.5425

				67.66		100.5425

				67.68		100.5425

				67.71		100.5425

				67.73		100.5425

				67.75		100.5425

				67.77		100.5425

				67.79		100.5425

				67.81		100.5425

				67.83		100.5425

				67.85		100.5425

				67.87		100.5425

				67.89		100.5425

				67.91		100.5425

				67.93		100.5425

				67.95		100.5425

				67.98		100.5425

				68		100.5425

				68.02		100.5425

				68.04		100.5425

				68.06		100.5425

				68.08		100.5425

				68.1		100.5425

				68.12		100.5425

				68.14		100.5425

				68.16		100.5425

				68.18		100.5425

				68.2		100.5425

				68.23		100.5425

				68.25		100.5425

				68.27		100.5425

				68.29		100.5425

				68.31		100.5425

				68.33		100.5425

				68.35		100.5425

				68.37		100.5425

				68.39		100.5425

				68.41		100.5425

				68.43		100.5425

				68.45		100.5425

				68.47		100.5367

				68.5		100.5367

				68.52		100.5367

				68.54		100.5367

				68.56		100.5367

				68.58		100.5367

				68.6		100.5367

				68.62		100.5425

				68.64		100.5367

				68.66		100.5425

				68.68		100.5425

				68.7		100.5425

				68.72		100.5425

				68.75		100.5425

				68.77		100.5425

				68.79		100.5367

				68.81		100.5425

				68.83		100.5367

				68.85		100.5367

				68.87		100.5367

				68.89		100.5367

				68.91		100.5367

				68.93		100.5367

				68.95		100.5367

				68.97		100.5367

				68.99		100.5367

				69.02		100.5367

				69.04		100.5425

				69.06		100.5425

				69.08		100.5425

				69.1		100.5425

				69.12		100.5425

				69.14		100.5425

				69.16		100.5425

				69.18		100.5425

				69.2		100.5425

				69.22		100.5425

				69.25		100.5425

				69.27		100.5425

				69.29		100.5425

				69.31		100.5425

				69.33		100.5425

				69.35		100.5425

				69.37		100.5425

				69.39		100.5425

				69.41		100.5425

				69.43		100.5425

				69.45		100.5425

				69.47		100.5425

				69.5		100.5425

				69.52		100.5425

				69.54		100.5483

				69.56		100.5483

				69.58		100.5483

				69.6		100.5483

				69.62		100.5483

				69.64		100.5483

				69.66		100.5483

				69.68		100.5483

				69.7		100.5483

				69.72		100.5483

				69.75		100.5483

				69.77		100.5483

				69.79		100.5483

				69.81		100.5483

				69.83		100.5483

				69.85		100.5483

				69.87		100.5483

				69.89		100.5483

				69.91		100.5483

				69.93		100.5483

				69.95		100.5483

				69.98		100.5483

				70		100.5483

				70.02		100.5483

				70.04		100.5483

				70.06		100.5483

				70.08		100.5483

				70.1		100.5483

				70.12		100.5483

				70.14		100.5483

				70.16		100.5483

				70.18		100.5483

				70.2		100.5483

				70.23		100.5483

				70.25		100.5483

				70.27		100.5483

				70.29		100.5483

				70.31		100.5483

				70.33		100.5483

				70.35		100.554

				70.37		100.554

				70.39		100.5483

				70.41		100.554

				70.43		100.554

				70.46		100.554

				70.48		100.554

				70.5		100.554

				70.52		100.554

				70.54		100.554

				70.56		100.554

				70.58		100.554

				70.6		100.554

				70.62		100.554

				70.64		100.554

				70.66		100.554

				70.68		100.554

				70.71		100.554

				70.73		100.554

				70.75		100.554

				70.77		100.5598

				70.79		100.554

				70.81		100.554

				70.83		100.554

				70.85		100.5598

				70.87		100.554

				70.89		100.5598

				70.91		100.554

				70.94		100.5598

				70.96		100.5598

				70.98		100.5598

				71		100.5598

				71.02		100.5598

				71.04		100.5598

				71.06		100.5598

				71.08		100.5598

				71.1		100.5598

				71.12		100.5598

				71.14		100.5598

				71.17		100.5598

				71.19		100.5598

				71.21		100.5598

				71.23		100.5598

				71.25		100.5598

				71.27		100.5598

				71.29		100.5598

				71.31		100.5598

				71.33		100.5598

				71.35		100.5598

				71.37		100.5598

				71.4		100.5598

				71.42		100.5598

				71.44		100.5598

				71.46		100.5598

				71.48		100.5598

				71.5		100.5598

				71.52		100.5598

				71.54		100.5598

				71.56		100.5598

				71.58		100.5598

				71.6		100.5598

				71.63		100.5598

				71.65		100.554

				71.67		100.554

				71.69		100.554

				71.71		100.554

				71.73		100.554

				71.75		100.554

				71.77		100.5598

				71.79		100.5598

				71.81		100.5598

				71.83		100.5598

				71.86		100.5598

				71.88		100.5598

				71.9		100.5598

				71.92		100.5598

				71.94		100.5598

				71.96		100.5598

				71.98		100.5598

				72		100.5598

				72.02		100.5598

				72.04		100.5598

				72.07		100.5598

				72.09		100.5598

				72.11		100.5598

				72.13		100.5598

				72.15		100.5598

				72.17		100.554

				72.19		100.5598

				72.21		100.5598

				72.23		100.5598

				72.25		100.554

				72.27		100.5598

				72.3		100.5598

				72.32		100.5598

				72.34		100.5598

				72.36		100.5598

				72.38		100.5598

				72.4		100.5598

				72.42		100.5598

				72.44		100.5598

				72.46		100.5598

				72.48		100.5598

				72.51		100.5598

				72.53		100.5598

				72.55		100.5598

				72.57		100.5598

				72.59		100.5598

				72.61		100.5598

				72.63		100.5598

				72.65		100.5598

				72.67		100.5598

				72.69		100.5598

				72.71		100.5598

				72.74		100.5598

				72.76		100.5598

				72.78		100.5598

				72.8		100.5598

				72.82		100.5598

				72.84		100.5598

				72.86		100.5598

				72.88		100.5598

				72.9		100.5598

				72.92		100.5598

				72.95		100.5598

				72.97		100.5598

				72.99		100.5598

				73.01		100.5598

				73.03		100.5598

				73.05		100.5598

				73.07		100.5598

				73.09		100.5598

				73.11		100.5598

				73.13		100.5598

				73.16		100.5598

				73.18		100.5598

				73.2		100.5598

				73.22		100.5598

				73.24		100.5598

				73.26		100.5598

				73.28		100.5598

				73.3		100.5598

				73.32		100.5598

				73.34		100.5598

				73.36		100.5598

				73.39		100.5598

				73.41		100.5598

				73.43		100.5598

				73.45		100.5656

				73.47		100.5656

				73.49		100.5656

				73.51		100.5656

				73.53		100.5656

				73.55		100.5656

				73.57		100.5656

				73.6		100.5598

				73.62		100.5656

				73.64		100.5656

				73.66		100.5656

				73.68		100.5656

				73.7		100.5656

				73.72		100.5656

				73.74		100.5656

				73.76		100.5656

				73.78		100.5656

				73.81		100.5656

				73.83		100.5656

				73.85		100.5656

				73.87		100.5656

				73.89		100.5656

				73.91		100.5656

				73.93		100.5656

				73.95		100.5656

				73.97		100.5656

				73.99		100.5656

				74.02		100.5656

				74.04		100.5656

				74.06		100.5656

				74.08		100.5656

				74.1		100.5656

				74.12		100.5656

				74.14		100.5656

				74.16		100.5598

				74.18		100.5656

				74.2		100.5656

				74.22		100.5656

				74.25		100.5656

				74.27		100.5656

				74.29		100.5656

				74.31		100.5656

				74.33		100.5656

				74.35		100.5656

				74.37		100.5656

				74.39		100.5598

				74.41		100.5656

				74.43		100.5598

				74.46		100.5598

				74.48		100.5598

				74.5		100.5656

				74.52		100.5598

				74.54		100.5656

				74.56		100.5598

				74.58		100.5598

				74.6		100.5598

				74.62		100.5598

				74.64		100.5598

				74.67		100.5598

				74.69		100.5598

				74.71		100.5598

				74.73		100.5598

				74.75		100.5598

				74.77		100.5598

				74.79		100.5598

				74.81		100.5598

				74.83		100.5598

				74.85		100.5598

				74.88		100.5598

				74.9		100.5598

				74.92		100.5598

				74.94		100.5598

				74.96		100.5598

				74.98		100.5598

				75		100.5598

				75.02		100.5598

				75.04		100.5598

				75.06		100.5598

				75.09		100.5598

				75.11		100.5598

				75.13		100.5598

				75.15		100.5598

				75.17		100.5598

				75.19		100.5598

				75.21		100.5598

				75.23		100.5598

				75.25		100.5598

				75.27		100.5598

				75.3		100.5598

				75.32		100.5598

				75.34		100.5598

				75.36		100.5598

				75.38		100.5598

				75.4		100.5598

				75.42		100.5598

				75.44		100.5598

				75.46		100.5598

				75.48		100.5598

				75.51		100.5598

				75.53		100.5598

				75.55		100.5598

				75.57		100.5598

				75.59		100.5598

				75.61		100.5598

				75.63		100.5598

				75.65		100.5598

				75.67		100.5598

				75.69		100.5598

				75.72		100.5598

				75.74		100.5598

				75.76		100.5598

				75.78		100.5598

				75.8		100.5598

				75.82		100.5598

				75.84		100.5598

				75.86		100.5598

				75.88		100.5598

				75.9		100.5598

				75.93		100.5598

				75.95		100.5598

				75.97		100.5598

				75.99		100.5598

				76.01		100.5598

				76.03		100.5598

				76.05		100.5598

				76.07		100.5598

				76.09		100.5598

				76.11		100.5598

				76.14		100.5598

				76.16		100.5598

				76.18		100.5656

				76.2		100.5598

				76.22		100.5598

				76.24		100.5598

				76.26		100.5598

				76.28		100.5598

				76.3		100.5598

				76.32		100.5598

				76.35		100.5656

				76.37		100.5598

				76.39		100.5598

				76.41		100.5656

				76.43		100.5598

				76.45		100.5598

				76.47		100.5598

				76.49		100.5598

				76.51		100.5598

				76.53		100.5598

				76.56		100.5598

				76.58		100.5598

				76.6		100.5656

				76.62		100.5598

				76.64		100.5598

				76.66		100.5656

				76.68		100.5656

				76.7		100.5656

				76.72		100.5656

				76.74		100.5656

				76.77		100.5656

				76.79		100.5656

				76.81		100.5656

				76.83		100.5656

				76.85		100.5656

				76.87		100.5656

				76.89		100.5656

				76.91		100.5598

				76.93		100.5656

				76.96		100.5656

				76.98		100.5656

				77		100.5656

				77.02		100.5656

				77.04		100.5656

				77.06		100.5656

				77.08		100.5656

				77.1		100.5656

				77.12		100.5656

				77.14		100.5656

				77.17		100.5656

				77.19		100.5656

				77.21		100.5656

				77.23		100.5656

				77.25		100.5656

				77.27		100.5656

				77.29		100.5656

				77.31		100.5656

				77.33		100.5656

				77.36		100.5656

				77.38		100.5656

				77.4		100.5656

				77.42		100.5656

				77.44		100.5656

				77.46		100.5656

				77.48		100.5656

				77.5		100.5656

				77.52		100.5656

				77.54		100.5656

				77.57		100.5656

				77.59		100.5656

				77.61		100.5656

				77.63		100.5656

				77.65		100.5656

				77.67		100.5656

				77.69		100.5656

				77.71		100.5656

				77.73		100.5656

				77.75		100.5656

				77.78		100.5656

				77.8		100.5656

				77.82		100.5656

				77.84		100.5656

				77.86		100.5656

				77.88		100.5656

				77.9		100.5656

				77.92		100.5656

				77.94		100.5656

				77.97		100.5656

				77.99		100.5656

				78.01		100.5656

				78.03		100.5656

				78.05		100.5656

				78.07		100.5656

				78.09		100.5656

				78.11		100.5656

				78.13		100.5656

				78.15		100.5656

				78.18		100.5656

				78.2		100.5656

				78.22		100.5656

				78.24		100.5656

				78.26		100.5656

				78.28		100.5656

				78.3		100.5656

				78.32		100.5656

				78.34		100.5656

				78.37		100.5656

				78.39		100.5656

				78.41		100.5656

				78.43		100.5656

				78.45		100.5656

				78.47		100.5656

				78.49		100.5656

				78.51		100.5656

				78.53		100.5656

				78.55		100.5656

				78.58		100.5656

				78.6		100.5656

				78.62		100.5656

				78.64		100.5656

				78.66		100.5656

				78.68		100.5656

				78.7		100.5656

				78.72		100.5656

				78.74		100.5656

				78.77		100.5656

				78.79		100.5656

				78.81		100.5656

				78.83		100.5656

				78.85		100.5656

				78.87		100.5656

				78.89		100.5656

				78.91		100.5656

				78.93		100.5656

				78.95		100.5656

				78.98		100.5656

				79		100.5656

				79.02		100.5656

				79.04		100.5656

				79.06		100.5656

				79.08		100.5656

				79.1		100.5656

				79.12		100.5656

				79.14		100.5656

				79.17		100.5656

				79.19		100.5656

				79.21		100.5598

				79.23		100.5598

				79.25		100.5598

				79.27		100.5598

				79.29		100.5598

				79.31		100.5656

				79.33		100.5598

				79.35		100.5598

				79.38		100.5598

				79.4		100.5598

				79.42		100.5598

				79.44		100.5598

				79.46		100.5598

				79.48		100.5598

				79.5		100.5598

				79.52		100.5598

				79.54		100.5598

				79.57		100.5598

				79.59		100.5598

				79.61		100.5598

				79.63		100.5598

				79.65		100.5598

				79.67		100.5598

				79.69		100.5598

				79.71		100.5598

				79.73		100.5598

				79.75		100.5598

				79.78		100.5598

				79.8		100.554

				79.82		100.5598

				79.84		100.554

				79.86		100.554

				79.88		100.554

				79.9		100.554

				79.92		100.554

				79.94		100.554

				79.97		100.554

				79.99		100.554

				80.01		100.554

				80.03		100.554

				80.05		100.554

				80.07		100.554

				80.09		100.554

				80.11		100.5598

				80.13		100.554

				80.15		100.5598

				80.18		100.5598

				80.2		100.5598

				80.22		100.5598

				80.24		100.5598

				80.26		100.554

				80.28		100.554

				80.3		100.554

				80.32		100.554

				80.34		100.554

				80.37		100.554

				80.39		100.554

				80.41		100.554

				80.43		100.554

				80.45		100.554

				80.47		100.554

				80.49		100.554

				80.51		100.554

				80.53		100.554

				80.56		100.554

				80.58		100.554

				80.6		100.554

				80.62		100.554

				80.64		100.554

				80.66		100.554

				80.68		100.5598

				80.7		100.5598

				80.72		100.554

				80.74		100.554

				80.77		100.5598

				80.79		100.554

				80.81		100.554

				80.83		100.554

				80.85		100.554

				80.87		100.554

				80.89		100.554

				80.91		100.554

				80.93		100.554

				80.96		100.554

				80.98		100.554

				81		100.554

				81.02		100.554

				81.04		100.554

				81.06		100.554

				81.08		100.554

				81.1		100.554

				81.12		100.5598

				81.14		100.5598

				81.17		100.5598

				81.19		100.5598

				81.21		100.5598

				81.23		100.5598

				81.25		100.5598

				81.27		100.5598

				81.29		100.5598

				81.31		100.5598

				81.33		100.5598

				81.36		100.5598

				81.38		100.5598

				81.4		100.5598

				81.42		100.5598

				81.44		100.5598

				81.46		100.5598

				81.48		100.5598

				81.5		100.5656

				81.52		100.5656

				81.54		100.5656

				81.57		100.5656

				81.59		100.5656

				81.61		100.5656

				81.63		100.5656

				81.65		100.5656

				81.67		100.5656

				81.69		100.5656

				81.71		100.5656

				81.73		100.5656

				81.76		100.5656

				81.78		100.5656

				81.8		100.5656

				81.82		100.5656

				81.84		100.5656

				81.86		100.5656

				81.88		100.5714

				81.9		100.5656

				81.92		100.5714

				81.94		100.5714

				81.97		100.5714

				81.99		100.5714

				82.01		100.5714

				82.03		100.5714

				82.05		100.5714

				82.07		100.5714

				82.09		100.5714

				82.11		100.5714

				82.13		100.5714

				82.16		100.5714

				82.18		100.5714

				82.2		100.5714

				82.22		100.5714

				82.24		100.5714

				82.26		100.5714

				82.28		100.5714

				82.3		100.5714

				82.32		100.5714

				82.35		100.5771

				82.37		100.5771

				82.39		100.5771

				82.41		100.5771

				82.43		100.5771

				82.45		100.5771

				82.47		100.5771

				82.49		100.5771

				82.51		100.5771

				82.53		100.5771

				82.56		100.5771

				82.58		100.5771

				82.6		100.5771

				82.62		100.5829

				82.64		100.5829

				82.66		100.5829

				82.68		100.5829

				82.7		100.5829

				82.72		100.5829

				82.75		100.5829

				82.77		100.5829

				82.79		100.5829

				82.81		100.5829

				82.83		100.5829

				82.85		100.5829

				82.87		100.5829

				82.89		100.5829

				82.91		100.5829

				82.93		100.5829

				82.96		100.5829

				82.98		100.5829

				83		100.5829

				83.02		100.5829

				83.04		100.5829

				83.06		100.5887

				83.08		100.5829

				83.1		100.5887

				83.12		100.5887

				83.15		100.5887

				83.17		100.5887

				83.19		100.5887

				83.21		100.5887

				83.23		100.5887

				83.25		100.5829

				83.27		100.5829

				83.29		100.5829

				83.31		100.5829

				83.33		100.5829

				83.36		100.5829

				83.38		100.5887

				83.4		100.5887

				83.42		100.5887

				83.44		100.5887

				83.46		100.5887

				83.48		100.5887

				83.5		100.5887

				83.52		100.5887

				83.55		100.5887

				83.57		100.5887

				83.59		100.5887

				83.61		100.5887

				83.63		100.5887

				83.65		100.5887

				83.67		100.5887

				83.69		100.5887

				83.71		100.5887

				83.74		100.5887

				83.76		100.5887

				83.78		100.5887

				83.8		100.5887

				83.82		100.5887

				83.84		100.5887

				83.86		100.5887

				83.88		100.5887

				83.9		100.5887

				83.92		100.5887

				83.95		100.5887

				83.97		100.5887

				83.99		100.5887

				84.01		100.5887

				84.03		100.5887

				84.05		100.5887

				84.07		100.5887

				84.09		100.5887

				84.11		100.5887

				84.14		100.5887

				84.16		100.5887

				84.18		100.5887

				84.2		100.5887

				84.22		100.5887

				84.24		100.5887

				84.26		100.5887

				84.28		100.5887

				84.3		100.5887

				84.32		100.5887

				84.35		100.5887

				84.37		100.5887

				84.39		100.5887

				84.41		100.5887

				84.43		100.5887

				84.45		100.5887

				84.47		100.5887

				84.49		100.5887

				84.51		100.5887

				84.54		100.5887

				84.56		100.5829

				84.58		100.5829

				84.6		100.5829

				84.62		100.5829

				84.64		100.5829

				84.66		100.5829

				84.68		100.5829

				84.7		100.5829

				84.73		100.5829

				84.75		100.5829

				84.77		100.5829

				84.79		100.5829

				84.81		100.5829

				84.83		100.5829

				84.85		100.5829

				84.87		100.5829

				84.89		100.5829

				84.91		100.5829

				84.94		100.5829

				84.96		100.5829

				84.98		100.5829

				85		100.5829

				85.02		100.5829

				85.04		100.5829

				85.06		100.5829

				85.08		100.5829

				85.1		100.5829

				85.13		100.5829

				85.15		100.5829

				85.17		100.5829

				85.19		100.5829

				85.21		100.5771

				85.23		100.5829

				85.25		100.5829

				85.27		100.5829

				85.29		100.5829

				85.31		100.5829

				85.34		100.5829

				85.36		100.5829

				85.38		100.5829

				85.4		100.5829

				85.42		100.5829

				85.44		100.5829

				85.46		100.5829

				85.48		100.5829

				85.5		100.5829

				85.53		100.5829

				85.55		100.5829

				85.57		100.5829

				85.59		100.5829

				85.61		100.5829

				85.63		100.5829

				85.65		100.5829

				85.67		100.5829

				85.69		100.5829

				85.72		100.5829

				85.74		100.5829

				85.76		100.5829

				85.78		100.5829

				85.8		100.5829

				85.82		100.5829

				85.84		100.5829

				85.86		100.5829

				85.88		100.5829

				85.9		100.5829

				85.93		100.5829

				85.95		100.5829

				85.97		100.5829

				85.99		100.5887

				86.01		100.5887

				86.03		100.5887

				86.05		100.5829

				86.07		100.5829

				86.09		100.5829

				86.12		100.5829

				86.14		100.5829

				86.16		100.5829

				86.18		100.5829

				86.2		100.5829

				86.22		100.5829

				86.24		100.5829

				86.26		100.5829

				86.28		100.5829

				86.31		100.5829

				86.33		100.5829

				86.35		100.5829

				86.37		100.5829

				86.39		100.5829

				86.41		100.5829

				86.43		100.5829

				86.45		100.5829

				86.47		100.5829

				86.49		100.5829

				86.52		100.5829

				86.54		100.5829

				86.56		100.5829

				86.58		100.5829

				86.6		100.5887

				86.62		100.5887

				86.64		100.5887

				86.66		100.5887

				86.68		100.5887

				86.71		100.5887

				86.73		100.5887

				86.75		100.5887

				86.77		100.5887

				86.79		100.5887

				86.81		100.5887

				86.83		100.5887

				86.85		100.5887

				86.87		100.5887

				86.9		100.5887

				86.92		100.5887

				86.94		100.5887

				86.96		100.5887

				86.98		100.5887

				87		100.5887

				87.02		100.5887

				87.04		100.5887

				87.06		100.5887

				87.08		100.5887

				87.11		100.5887

				87.13		100.5887

				87.15		100.5887

				87.17		100.5887

				87.19		100.5887

				87.21		100.5887

				87.23		100.5887

				87.25		100.5887

				87.27		100.5887

				87.3		100.5887

				87.32		100.5887

				87.34		100.5887

				87.36		100.5887

				87.38		100.5887

				87.4		100.5887

				87.42		100.5887

				87.44		100.5887

				87.46		100.5887

				87.48		100.5887

				87.51		100.5887

				87.53		100.5887

				87.55		100.5887

				87.57		100.5887

				87.59		100.5887

				87.61		100.5887

				87.63		100.5887

				87.65		100.5887

				87.67		100.5887

				87.7		100.5887

				87.72		100.5887

				87.74		100.5887

				87.76		100.5887

				87.78		100.5887

				87.8		100.5887

				87.82		100.5887

				87.84		100.5887

				87.86		100.5887

				87.88		100.5887

				87.91		100.5887

				87.93		100.5887

				87.95		100.5887

				87.97		100.5887

				87.99		100.5887

				88.01		100.5887

				88.03		100.5887

				88.05		100.5887

				88.07		100.5887

				88.1		100.5887

				88.12		100.5887

				88.14		100.5887

				88.16		100.5887

				88.18		100.5887

				88.2		100.5887

				88.22		100.5887

				88.24		100.5887

				88.26		100.5887

				88.28		100.5887

				88.31		100.5887

				88.33		100.5887

				88.35		100.5887

				88.37		100.5887

				88.39		100.5887

				88.41		100.5887

				88.43		100.5887

				88.45		100.5887

				88.47		100.5887

				88.5		100.5887

				88.52		100.5887

				88.54		100.5887

				88.56		100.5887

				88.58		100.5887

				88.6		100.5887

				88.62		100.5887

				88.64		100.5887

				88.66		100.5887

				88.69		100.5887

				88.71		100.5887

				88.73		100.5887

				88.75		100.5887

				88.77		100.5887

				88.79		100.5887

				88.81		100.5887

				88.83		100.5887

				88.85		100.5887

				88.87		100.5887

				88.9		100.5887

				88.92		100.5887

				88.94		100.5887

				88.96		100.5887

				88.98		100.5887

				89		100.5887

				89.02		100.5887

				89.04		100.5887

				89.06		100.5887

				89.09		100.5887

				89.11		100.5887

				89.13		100.5887

				89.15		100.5887

				89.17		100.5887

				89.19		100.5887

				89.21		100.5887

				89.23		100.5887

				89.25		100.5887

				89.27		100.5887

				89.3		100.5887

				89.32		100.5887

				89.34		100.5887

				89.36		100.5887

				89.38		100.5887

				89.4		100.5829

				89.42		100.5829

				89.44		100.5829

				89.46		100.5829

				89.49		100.5829

				89.51		100.5829

				89.53		100.5829

				89.55		100.5829

				89.57		100.5829

				89.59		100.5829

				89.61		100.5829

				89.63		100.5829

				89.65		100.5829

				89.67		100.5887

				89.7		100.5887

				89.72		100.5887

				89.74		100.5887

				89.76		100.5887

				89.78		100.5887

				89.8		100.5887

				89.82		100.5887

				89.84		100.5887

				89.86		100.5829

				89.89		100.5887

				89.91		100.5887

				89.93		100.5887

				89.95		100.5887

				89.97		100.5887

				89.99		100.5829

				90.01		100.5887

				90.03		100.5887

				90.05		100.5887

				90.07		100.5887

				90.1		100.5887

				90.12		100.5887

				90.14		100.5887

				90.16		100.5887

				90.18		100.5887

				90.2		100.5887

				90.22		100.5887

				90.24		100.5887

				90.26		100.5887

				90.29		100.5887

				90.31		100.5887

				90.33		100.5887

				90.35		100.5887

				90.37		100.5887

				90.39		100.5887

				90.41		100.5887

				90.43		100.5887

				90.45		100.5887

				90.47		100.5887

				90.5		100.5887

				90.52		100.5944

				90.54		100.5944

				90.56		100.5944

				90.58		100.5944

				90.6		100.5944

				90.62		100.5944

				90.64		100.5944

				90.66		100.5944

				90.69		100.5944

				90.71		100.5944

				90.73		100.5944

				90.75		100.5944

				90.77		100.5944

				90.79		100.5944

				90.81		100.5944

				90.83		100.5944

				90.85		100.5944

				90.87		100.5944

				90.9		100.5944

				90.92		100.5944

				90.94		100.5944

				90.96		100.5944

				90.98		100.5944

				91		100.5944

				91.02		100.5944

				91.04		100.6002

				91.06		100.6002

				91.09		100.6002

				91.11		100.6002

				91.13		100.6002

				91.15		100.6002

				91.17		100.6002

				91.19		100.6002

				91.21		100.6002

				91.23		100.6002

				91.25		100.5944

				91.27		100.6002

				91.3		100.5944

				91.32		100.5944

				91.34		100.5944

				91.36		100.5944

				91.38		100.5944

				91.4		100.5944

				91.42		100.5944

				91.44		100.5944

				91.46		100.5944

				91.49		100.6002

				91.51		100.6002

				91.53		100.6002

				91.55		100.6002

				91.57		100.6002

				91.59		100.6002

				91.61		100.6002

				91.63		100.6002

				91.65		100.6002

				91.67		100.6002

				91.7		100.6002

				91.72		100.6002

				91.74		100.6002

				91.76		100.5944

				91.78		100.5944

				91.8		100.5944

				91.82		100.5944

				91.84		100.5944

				91.86		100.5944

				91.89		100.5944

				91.91		100.5944

				91.93		100.5944

				91.95		100.5944

				91.97		100.5944

				91.99		100.5944

				92.01		100.5944

				92.03		100.5944

				92.05		100.5944

				92.07		100.5944

				92.1		100.5944

				92.12		100.5944

				92.14		100.5944

				92.16		100.5944

				92.18		100.5944

				92.2		100.5944

				92.22		100.5944

				92.24		100.5944

				92.26		100.5944

				92.29		100.5887

				92.31		100.5887

				92.33		100.5887

				92.35		100.5887

				92.37		100.5944

				92.39		100.5944

				92.41		100.5887

				92.43		100.5944

				92.45		100.5887

				92.47		100.5887

				92.5		100.5887

				92.52		100.5887

				92.54		100.5887

				92.56		100.5887

				92.58		100.5887

				92.6		100.5887

				92.62		100.5887

				92.64		100.5887

				92.66		100.5887

				92.69		100.5887

				92.71		100.5887

				92.73		100.5887

				92.75		100.5887

				92.77		100.5887

				92.79		100.5887

				92.81		100.5887

				92.83		100.5887

				92.85		100.5887

				92.87		100.5887

				92.9		100.5887

				92.92		100.5887

				92.94		100.5887

				92.96		100.5887

				92.98		100.5887

				93		100.5887

				93.02		100.5887

				93.04		100.5887

				93.06		100.5829

				93.09		100.5829

				93.11		100.5829

				93.13		100.5829

				93.15		100.5829

				93.17		100.5829

				93.19		100.5829

				93.21		100.5829

				93.23		100.5829

				93.25		100.5829

				93.27		100.5829

				93.3		100.5829

				93.32		100.5829

				93.34		100.5829

				93.36		100.5829

				93.38		100.5829

				93.4		100.5829

				93.42		100.5887

				93.44		100.5829

				93.46		100.5829

				93.49		100.5829

				93.51		100.5829

				93.53		100.5829

				93.55		100.5829

				93.57		100.5829

				93.59		100.5829

				93.61		100.5829

				93.63		100.5829

				93.65		100.5829

				93.67		100.5829

				93.7		100.5887

				93.72		100.5829

				93.74		100.5829

				93.76		100.5829

				93.78		100.5829

				93.8		100.5829

				93.82		100.5829

				93.84		100.5829

				93.86		100.5829

				93.89		100.5829

				93.91		100.5829

				93.93		100.5829

				93.95		100.5829

				93.97		100.5829

				93.99		100.5829

				94.01		100.5829

				94.03		100.5829

				94.05		100.5887

				94.07		100.5829

				94.1		100.5887

				94.12		100.5829

				94.14		100.5829

				94.16		100.5887

				94.18		100.5887

				94.2		100.5829

				94.22		100.5829

				94.24		100.5887

				94.26		100.5887

				94.28		100.5887

				94.31		100.5887

				94.33		100.5887

				94.35		100.5887

				94.37		100.5887

				94.39		100.5887

				94.41		100.5887

				94.43		100.5887

				94.45		100.5887

				94.47		100.5887

				94.5		100.5887

				94.52		100.5887

				94.54		100.5887

				94.56		100.5887

				94.58		100.5887

				94.6		100.5887

				94.62		100.5887

				94.64		100.5887

				94.66		100.5887

				94.68		100.5887

				94.71		100.5887

				94.73		100.5887

				94.75		100.5887

				94.77		100.5887

				94.79		100.5887

				94.81		100.5887

				94.83		100.5887

				94.85		100.5887

				94.87		100.5829

				94.9		100.5887

				94.92		100.5887

				94.94		100.5887

				94.96		100.5887

				94.98		100.5887

				95		100.5887

				95.02		100.5887

				95.04		100.5887

				95.06		100.5829

				95.08		100.5887

				95.11		100.5887

				95.13		100.5887

				95.15		100.5887

				95.17		100.5887

				95.19		100.5887

				95.21		100.5887

				95.23		100.5887

				95.25		100.5887

				95.27		100.5887

				95.3		100.5887

				95.32		100.5887

				95.34		100.5887

				95.36		100.5887

				95.38		100.5887

				95.4		100.5887

				95.42		100.5887

				95.44		100.5887

				95.46		100.5887

				95.48		100.5887

				95.51		100.5887

				95.53		100.5887

				95.55		100.5887

				95.57		100.5887

				95.59		100.5887

				95.61		100.5887

				95.63		100.5887

				95.65		100.5887

				95.67		100.5887

				95.7		100.5887

				95.72		100.5887

				95.74		100.5887

				95.76		100.5887

				95.78		100.5887

				95.8		100.5887

				95.82		100.5887

				95.84		100.5887

				95.86		100.5887

				95.89		100.5944

				95.91		100.5887

				95.93		100.5887

				95.95		100.5944

				95.97		100.5944

				95.99		100.5944

				96.01		100.5944

				96.03		100.5944

				96.05		100.5944

				96.07		100.5944

				96.1		100.5944

				96.12		100.5944

				96.14		100.5944

				96.16		100.5887

				96.18		100.5944

				96.2		100.5944

				96.22		100.5944

				96.24		100.5887

				96.26		100.5887

				96.29		100.5944

				96.31		100.5944

				96.33		100.5887

				96.35		100.5944

				96.37		100.5944

				96.39		100.5944

				96.41		100.5944

				96.43		100.5944

				96.45		100.5944

				96.47		100.5944

				96.5		100.5944

				96.52		100.5944

				96.54		100.5944

				96.56		100.5944

				96.58		100.5944

				96.6		100.5944

				96.62		100.5944

				96.64		100.5944

				96.66		100.5944

				96.69		100.5944

				96.71		100.5944

				96.73		100.5944

				96.75		100.5944

				96.77		100.5944

				96.79		100.5944

				96.81		100.5944

				96.83		100.5944

				96.85		100.5944

				96.87		100.5944

				96.9		100.5944

				96.92		100.5944

				96.94		100.6002

				96.96		100.6002

				96.98		100.5944

				97		100.6002

				97.02		100.6002

				97.04		100.6002

				97.06		100.6002

				97.09		100.6002

				97.11		100.6002

				97.13		100.5944

				97.15		100.6002

				97.17		100.5944

				97.19		100.5944

				97.21		100.5944

				97.23		100.5944

				97.25		100.5944

				97.27		100.5944

				97.3		100.5944

				97.32		100.5944

				97.34		100.5944

				97.36		100.5944

				97.38		100.5944

				97.4		100.5944

				97.42		100.5944

				97.44		100.5944

				97.46		100.5944

				97.49		100.5944

				97.51		100.5944

				97.53		100.5944

				97.55		100.5944

				97.57		100.5944

				97.59		100.5944

				97.61		100.5944

				97.63		100.5944

				97.65		100.5944

				97.67		100.5944

				97.7		100.5944

				97.72		100.5944

				97.74		100.5944

				97.76		100.5944

				97.78		100.5944

				97.8		100.5944

				97.82		100.5944

				97.84		100.5944

				97.86		100.5944

				97.89		100.5887

				97.91		100.5887

				97.93		100.5887

				97.95		100.5887

				97.97		100.5887

				97.99		100.5887

				98.01		100.5887

				98.03		100.5887

				98.05		100.5887

				98.07		100.5887

				98.1		100.5887

				98.12		100.5887

				98.14		100.5887

				98.16		100.5887

				98.18		100.5887

				98.2		100.5887

				98.22		100.5887

				98.24		100.5887

				98.26		100.5887

				98.29		100.5887

				98.31		100.5887

				98.33		100.5887

				98.35		100.5887

				98.37		100.5887

				98.39		100.5887

				98.41		100.5944

				98.43		100.5944

				98.45		100.5887

				98.47		100.5887

				98.5		100.5887

				98.52		100.5887

				98.54		100.5887

				98.56		100.5887

				98.58		100.5887

				98.6		100.5887

				98.62		100.5887

				98.64		100.5887

				98.66		100.5887

				98.69		100.5887

				98.71		100.5887

				98.73		100.5887

				98.75		100.5887

				98.77		100.5887

				98.79		100.5887

				98.81		100.5887

				98.83		100.5887

				98.85		100.5887

				98.87		100.5887

				98.9		100.5887

				98.92		100.5887

				98.94		100.5887

				98.96		100.5887

				98.98		100.5887

				99		100.5887

				99.02		100.5887

				99.04		100.5887

				99.06		100.5887

				99.09		100.5887

				99.11		100.5887

				99.13		100.5887

				99.15		100.5887

				99.17		100.5887

				99.19		100.5887

				99.21		100.5887

				99.23		100.5887

				99.25		100.5887

				99.27		100.5887

				99.3		100.5887

				99.32		100.5887

				99.34		100.5887

				99.36		100.5887

				99.38		100.5887

				99.4		100.5887

				99.42		100.5887

				99.44		100.5887

				99.46		100.5887

				99.49		100.5887

				99.51		100.5887

				99.53		100.5887

				99.55		100.5887

				99.57		100.5887

				99.59		100.5887

				99.61		100.5887

				99.63		100.5887

				99.65		100.5887

				99.67		100.5887

				99.7		100.5887

				99.72		100.5887

				99.74		100.5887

				99.76		100.5887

				99.78		100.5887

				99.8		100.5887

				99.82		100.5887

				99.84		100.5887

				99.86		100.5887

				99.89		100.5887

				99.91		100.5887

				99.93		100.5887

				99.95		100.5887

				99.97		100.5887

				99.99		100.5887

				100.01		100.5887

				100.03		100.5944

				100.05		100.5944

				100.07		100.5944

				100.1		100.5944

				100.12		100.5944

				100.14		100.5887

				100.16		100.5944

				100.18		100.5887

				100.2		100.5944

				100.22		100.5887

				100.24		100.5887

				100.26		100.5887

				100.28		100.5887

				100.31		100.5887

				100.33		100.5887

				100.35		100.5887

				100.37		100.5887

				100.39		100.5887

				100.41		100.5887

				100.43		100.5887

				100.45		100.5887

				100.47		100.5887

				100.5		100.5887

				100.52		100.5887

				100.54		100.5887

				100.56		100.5887

				100.58		100.5944

				100.6		100.5887

				100.62		100.5887

				100.64		100.5887

				100.66		100.5887

				100.68		100.5887

				100.71		100.5887

				100.73		100.5887

				100.75		100.5887

				100.77		100.5887

				100.79		100.5887

				100.81		100.5887

				100.83		100.5887

				100.85		100.5887

				100.87		100.5887

				100.9		100.5887

				100.92		100.5887

				100.94		100.5887

				100.96		100.5887

				100.98		100.5887

				101		100.5887

				101.02		100.5887

				101.04		100.5887

				101.06		100.5887

				101.08		100.5887

				101.11		100.5887

				101.13		100.5887

				101.15		100.5887

				101.17		100.5887

				101.19		100.5887

				101.21		100.5887

				101.23		100.5887

				101.25		100.5887

				101.27		100.5887

				101.29		100.5887

				101.32		100.5887

				101.34		100.5887

				101.36		100.5887

				101.38		100.5887

				101.4		100.5887

				101.42		100.5944

				101.44		100.5887

				101.46		100.5944

				101.48		100.5944

				101.51		100.5944

				101.53		100.5944

				101.55		100.5944

				101.57		100.5944

				101.59		100.5944

				101.61		100.5944

				101.63		100.5944

				101.65		100.5944

				101.67		100.5944

				101.69		100.5944

				101.72		100.5944

				101.74		100.5944

				101.76		100.5944

				101.78		100.5887

				101.8		100.5887

				101.82		100.5887

				101.84		100.5887

				101.86		100.5887

				101.88		100.5887

				101.91		100.5887

				101.93		100.5887

				101.95		100.5887

				101.97		100.5887

				101.99		100.5887

				102.01		100.5887

				102.03		100.5887

				102.05		100.5887

				102.07		100.5887

				102.09		100.5887

				102.12		100.5887

				102.14		100.5887

				102.16		100.5887

				102.18		100.5887

				102.2		100.5887

				102.22		100.5887

				102.24		100.5887

				102.26		100.5887

				102.28		100.5887

				102.3		100.5887

				102.33		100.5887

				102.35		100.5887

				102.37		100.5887

				102.39		100.5887

				102.41		100.5887

				102.43		100.5887

				102.45		100.5887

				102.47		100.5887

				102.49		100.5887

				102.52		100.5887

				102.54		100.5887

				102.56		100.5887

				102.58		100.5887

				102.6		100.5887

				102.62		100.5887

				102.64		100.5887

				102.66		100.5887

				102.68		100.5887

				102.7		100.5887

				102.73		100.5887

				102.75		100.5887

				102.77		100.5887

				102.79		100.5887

				102.81		100.5887

				102.83		100.5887

				102.85		100.5887

				102.87		100.5887

				102.89		100.5887

				102.92		100.5887

				102.94		100.5887

				102.96		100.5887

				102.98		100.5887

				103		100.5887

				103.02		100.5887

				103.04		100.5887

				103.06		100.5887

				103.08		100.5887

				103.1		100.5887

				103.13		100.5887

				103.15		100.5887

				103.17		100.5829

				103.19		100.5829

				103.21		100.5829

				103.23		100.5829

				103.25		100.5829

				103.27		100.5829

				103.29		100.5829

				103.32		100.5829

				103.34		100.5829

				103.36		100.5829

				103.38		100.5829

				103.4		100.5829

				103.42		100.5829

				103.44		100.5829

				103.46		100.5829

				103.48		100.5829

				103.5		100.5829

				103.53		100.5829

				103.55		100.5829

				103.57		100.5829

				103.59		100.5829

				103.61		100.5829

				103.63		100.5829

				103.65		100.5829

				103.67		100.5829

				103.69		100.5829

				103.71		100.5829

				103.74		100.5829

				103.76		100.5829

				103.78		100.5829

				103.8		100.5829

				103.82		100.5829

				103.84		100.5829

				103.86		100.5829

				103.88		100.5829

				103.9		100.5829

				103.93		100.5829

				103.95		100.5829

				103.97		100.5829

				103.99		100.5829

				104.01		100.5829

				104.03		100.5829

				104.05		100.5829

				104.07		100.5829

				104.09		100.5829

				104.11		100.5829

				104.14		100.5829

				104.16		100.5829

				104.18		100.5829

				104.2		100.5829

				104.22		100.5829

				104.24		100.5829

				104.26		100.5829

				104.28		100.5829

				104.3		100.5829

				104.32		100.5829

				104.35		100.5829

				104.37		100.5829

				104.39		100.5829

				104.41		100.5829

				104.43		100.5829

				104.45		100.5829

				104.47		100.5829

				104.49		100.5829

				104.51		100.5829

				104.54		100.5829

				104.56		100.5829

				104.58		100.5829

				104.6		100.5829

				104.62		100.5829

				104.64		100.5829

				104.66		100.5829

				104.68		100.5829

				104.7		100.5829

				104.72		100.5771

				104.75		100.5771

				104.77		100.5771

				104.79		100.5771

				104.81		100.5771

				104.83		100.5771

				104.85		100.5771

				104.87		100.5771

				104.89		100.5771

				104.91		100.5771

				104.93		100.5771

				104.96		100.5771

				104.98		100.5771

				105		100.5771

				105.02		100.5771

				105.04		100.5771

				105.06		100.5771

				105.08		100.5771

				105.1		100.5714

				105.12		100.5714

				105.14		100.5714

				105.17		100.5714

				105.19		100.5771

				105.21		100.5771

				105.23		100.5714

				105.25		100.5714

				105.27		100.5771

				105.29		100.5714

				105.31		100.5714

				105.33		100.5771

				105.36		100.5771

				105.38		100.5771

				105.4		100.5771

				105.42		100.5714

				105.44		100.5771

				105.46		100.5771

				105.48		100.5771

				105.5		100.5771

				105.52		100.5771

				105.54		100.5771

				105.57		100.5771

				105.59		100.5771

				105.61		100.5771

				105.63		100.5771

				105.65		100.5771

				105.67		100.5714

				105.69		100.5714

				105.71		100.5714

				105.73		100.5771

				105.75		100.5714

				105.78		100.5714

				105.8		100.5714

				105.82		100.5714

				105.84		100.5714

				105.86		100.5771

				105.88		100.5771

				105.9		100.5771

				105.92		100.5771

				105.94		100.5771

				105.97		100.5771

				105.99		100.5771

				106.01		100.5771

				106.03		100.5714

				106.05		100.5714

				106.07		100.5714

				106.09		100.5714

				106.11		100.5714

				106.13		100.5714

				106.15		100.5714

				106.18		100.5714

				106.2		100.5714

				106.22		100.5714

				106.24		100.5714

				106.26		100.5714

				106.28		100.5714

				106.3		100.5714

				106.32		100.5714

				106.34		100.5714

				106.36		100.5714

				106.39		100.5714

				106.41		100.5714

				106.43		100.5714

				106.45		100.5714

				106.47		100.5714

				106.49		100.5714

				106.51		100.5714

				106.53		100.5714

				106.55		100.5714

				106.58		100.5714

				106.6		100.5714

				106.62		100.5714

				106.64		100.5714

				106.66		100.5714

				106.68		100.5714

				106.7		100.5714

				106.72		100.5714

				106.74		100.5714

				106.76		100.5714

				106.79		100.5714

				106.81		100.5714

				106.83		100.5714

				106.85		100.5714

				106.87		100.5714

				106.89		100.5714

				106.91		100.5714

				106.93		100.5656

				106.95		100.5714

				106.97		100.5656

				107		100.5714

				107.02		100.5656

				107.04		100.5714

				107.06		100.5714

				107.08		100.5714

				107.1		100.5714

				107.12		100.5656

				107.14		100.5714

				107.16		100.5714

				107.18		100.5714

				107.21		100.5714

				107.23		100.5714

				107.25		100.5714

				107.27		100.5656

				107.29		100.5714

				107.31		100.5714

				107.33		100.5714

				107.35		100.5714

				107.37		100.5714

				107.4		100.5714

				107.42		100.5656

				107.44		100.5714

				107.46		100.5656

				107.48		100.5656

				107.5		100.5714

				107.52		100.5656

				107.54		100.5656

				107.56		100.5656

				107.58		100.5656

				107.61		100.5656

				107.63		100.5656

				107.65		100.5656

				107.67		100.5656

				107.69		100.5656

				107.71		100.5656

				107.73		100.5656

				107.75		100.5656

				107.77		100.5656

				107.79		100.5656

				107.82		100.5656

				107.84		100.5656

				107.86		100.5656

				107.88		100.5656

				107.9		100.5656

				107.92		100.5656

				107.94		100.5656

				107.96		100.5656

				107.98		100.5656

				108		100.5656

				108.03		100.5656

				108.05		100.5656

				108.07		100.5656

				108.09		100.5656

				108.11		100.5714

				108.13		100.5714

				108.15		100.5714

				108.17		100.5714

				108.19		100.5714

				108.22		100.5714

				108.24		100.5714

				108.26		100.5714

				108.28		100.5714

				108.3		100.5714

				108.32		100.5714

				108.34		100.5714

				108.36		100.5714

				108.38		100.5714

				108.4		100.5714

				108.43		100.5714

				108.45		100.5714

				108.47		100.5714

				108.49		100.5714

				108.51		100.5714

				108.53		100.5714

				108.55		100.5714

				108.57		100.5656

				108.59		100.5656

				108.61		100.5714

				108.64		100.5714

				108.66		100.5656

				108.68		100.5656

				108.7		100.5656

				108.72		100.5656

				108.74		100.5656

				108.76		100.5656

				108.78		100.5656

				108.8		100.5656

				108.83		100.5656

				108.85		100.5656

				108.87		100.5656

				108.89		100.5656

				108.91		100.5656

				108.93		100.5656

				108.95		100.5656

				108.97		100.5656

				108.99		100.5656

				109.01		100.5656

				109.04		100.5656

				109.06		100.5656

				109.08		100.5656

				109.1		100.5656

				109.12		100.5656

				109.14		100.5656

				109.16		100.5656

				109.18		100.5656

				109.2		100.5656

				109.22		100.5656

				109.25		100.5656

				109.27		100.5656

				109.29		100.5656

				109.31		100.5656

				109.33		100.5656

				109.35		100.5656

				109.37		100.5656

				109.39		100.5656

				109.41		100.5656

				109.43		100.5656

				109.46		100.5656

				109.48		100.5656

				109.5		100.5656

				109.52		100.5656

				109.54		100.5656

				109.56		100.5656

				109.58		100.5656

				109.6		100.5656

				109.62		100.5656

				109.64		100.5656

				109.67		100.5656

				109.69		100.5598

				109.71		100.5656

				109.73		100.5598

				109.75		100.5656

				109.77		100.5656

				109.79		100.5656

				109.81		100.5598

				109.83		100.5656

				109.86		100.5598

				109.88		100.5598

				109.9		100.5598

				109.92		100.5598

				109.94		100.5598

				109.96		100.5598

				109.98		100.5598

				110		100.5598

				110.02		100.5598

				110.04		100.5598

				110.07		100.554

				110.09		100.554

				110.11		100.554

				110.13		100.5598

				110.15		100.554

				110.17		100.554

				110.19		100.554

				110.21		100.554

				110.23		100.554

				110.25		100.554

				110.28		100.554

				110.3		100.554

				110.32		100.5483

				110.34		100.554

				110.36		100.5483

				110.38		100.5483

				110.4		100.5483

				110.42		100.5483

				110.44		100.5483

				110.46		100.5483

				110.49		100.5483

				110.51		100.5483

				110.53		100.5483

				110.55		100.5483

				110.57		100.5483

				110.59		100.5483

				110.61		100.5483

				110.63		100.5483

				110.65		100.5483

				110.68		100.5483

				110.7		100.5483

				110.72		100.5483

				110.74		100.5483

				110.76		100.5483

				110.78		100.5483

				110.8		100.5483

				110.82		100.5483

				110.84		100.5483

				110.86		100.5483

				110.89		100.5483

				110.91		100.5483

				110.93		100.5483

				110.95		100.5483

				110.97		100.5483

				110.99		100.5483

				111.01		100.5483

				111.03		100.5483

				111.05		100.5483

				111.08		100.5483

				111.1		100.5483

				111.12		100.5483

				111.14		100.5483

				111.16		100.5483

				111.18		100.5483

				111.2		100.5483

				111.22		100.5483

				111.24		100.5483

				111.26		100.5483

				111.29		100.5483

				111.31		100.5483

				111.33		100.5483

				111.35		100.5483

				111.37		100.5483

				111.39		100.5483

				111.41		100.5483

				111.43		100.5483

				111.45		100.5425

				111.48		100.5483

				111.5		100.5483

				111.52		100.5483

				111.54		100.5483

				111.56		100.5483

				111.58		100.5425

				111.6		100.5425

				111.62		100.5425

				111.64		100.5425

				111.66		100.5425

				111.69		100.5425

				111.71		100.5425

				111.73		100.5425

				111.75		100.5425

				111.77		100.5425

				111.79		100.5425

				111.81		100.5425

				111.83		100.5425

				111.85		100.5425

				111.87		100.5425

				111.9		100.5425

				111.92		100.5425

				111.94		100.5425

				111.96		100.5425

				111.98		100.5425

				112		100.5425

				112.02		100.5425

				112.04		100.5425

				112.06		100.5425

				112.09		100.5425

				112.11		100.5425

				112.13		100.5425

				112.15		100.5483

				112.17		100.5425

				112.19		100.5425

				112.21		100.5425

				112.23		100.5425

				112.25		100.5425

				112.27		100.5425

				112.3		100.5425

				112.32		100.5425

				112.34		100.5425

				112.36		100.5425

				112.38		100.5425

				112.4		100.5425

				112.42		100.5425

				112.44		100.5425

				112.46		100.5425

				112.48		100.5425

				112.51		100.5425

				112.53		100.5425

				112.55		100.5425

				112.57		100.5425

				112.59		100.5425

				112.61		100.5425

				112.63		100.5425

				112.65		100.5425

				112.67		100.5425

				112.7		100.5425

				112.72		100.5425

				112.74		100.5425

				112.76		100.5425

				112.78		100.5425

				112.8		100.5425

				112.82		100.5425

				112.84		100.5425

				112.86		100.5425

				112.88		100.5425

				112.91		100.5425

				112.93		100.5425

				112.95		100.5425

				112.97		100.5425

				112.99		100.5425

				113.01		100.5425

				113.03		100.5425

				113.05		100.5425

				113.07		100.5425

				113.09		100.5425

				113.12		100.5425

				113.14		100.5425

				113.16		100.5425

				113.18		100.5425

				113.2		100.5425

				113.22		100.5425

				113.24		100.5425

				113.26		100.5367

				113.28		100.5367

				113.31		100.5367

				113.33		100.5425

				113.35		100.5367

				113.37		100.5367

				113.39		100.5367

				113.41		100.5367

				113.43		100.5367

				113.45		100.5367

				113.47		100.5367

				113.49		100.5367

				113.52		100.5367

				113.54		100.5367

				113.56		100.5367

				113.58		100.5367

				113.6		100.5367

				113.62		100.5367

				113.64		100.5367

				113.66		100.5367

				113.68		100.5367

				113.71		100.531

				113.73		100.5367

				113.75		100.531

				113.77		100.5367

				113.79		100.531

				113.81		100.531

				113.83		100.531

				113.85		100.531

				113.87		100.531

				113.89		100.531

				113.92		100.531

				113.94		100.531

				113.96		100.531

				113.98		100.531

				114		100.531

				114.02		100.531

				114.04		100.531

				114.06		100.531

				114.08		100.531

				114.11		100.531

				114.13		100.531

				114.15		100.531

				114.17		100.531

				114.19		100.5252

				114.21		100.5252

				114.23		100.5252

				114.25		100.5252

				114.27		100.5252

				114.29		100.5252

				114.32		100.5252

				114.34		100.5252

				114.36		100.5252

				114.38		100.5252

				114.4		100.5252

				114.42		100.5252

				114.44		100.5252

				114.46		100.5252

				114.48		100.5252

				114.5		100.5252

				114.53		100.5252

				114.55		100.5252

				114.57		100.5252

				114.59		100.5252

				114.61		100.5252

				114.63		100.5252

				114.65		100.5252

				114.67		100.5252

				114.69		100.5252

				114.72		100.5252

				114.74		100.5252

				114.76		100.5252

				114.78		100.5252

				114.8		100.5252

				114.82		100.5252

				114.84		100.5252

				114.86		100.5252

				114.88		100.5252

				114.9		100.5194

				114.93		100.5194

				114.95		100.5194

				114.97		100.5194

				114.99		100.5194

				115.01		100.5194

				115.03		100.5194

				115.05		100.5194

				115.07		100.5194

				115.09		100.5194

				115.11		100.5194

				115.14		100.5194

				115.16		100.5194

				115.18		100.5194

				115.2		100.5194

				115.22		100.5194

				115.24		100.5194

				115.26		100.5194

				115.28		100.5194

				115.3		100.5194

				115.33		100.5194

				115.35		100.5194

				115.37		100.5194

				115.39		100.5194

				115.41		100.5194

				115.43		100.5194

				115.45		100.5194

				115.47		100.5194

				115.49		100.5194

				115.51		100.5194

				115.54		100.5194

				115.56		100.5194

				115.58		100.5194

				115.6		100.5136

				115.62		100.5194

				115.64		100.5194

				115.66		100.5136

				115.68		100.5194

				115.7		100.5136

				115.72		100.5136

				115.75		100.5194

				115.77		100.5136

				115.79		100.5136

				115.81		100.5136

				115.83		100.5136

				115.85		100.5136

				115.87		100.5136

				115.89		100.5136

				115.91		100.5136

				115.93		100.5136

				115.96		100.5136

				115.98		100.5136

				116		100.5136

				116.02		100.5136

				116.04		100.5136

				116.06		100.5136

				116.08		100.5136

				116.1		100.5136

				116.12		100.5136

				116.15		100.5136

				116.17		100.5136

				116.19		100.5136

				116.21		100.5136

				116.23		100.5136

				116.25		100.5136

				116.27		100.5079

				116.29		100.5079

				116.31		100.5079

				116.33		100.5079

				116.36		100.5079

				116.38		100.5079

				116.4		100.5079

				116.42		100.5079

				116.44		100.5079

				116.46		100.5079

				116.48		100.5079

				116.5		100.5079

				116.52		100.5079

				116.54		100.5079

				116.57		100.5079

				116.59		100.5079

				116.61		100.5079

				116.63		100.5079

				116.65		100.5021

				116.67		100.5079

				116.69		100.5021

				116.71		100.5021

				116.73		100.5021

				116.75		100.5021

				116.78		100.5021

				116.8		100.5021

				116.82		100.5021

				116.84		100.5021

				116.86		100.5021

				116.88		100.5021

				116.9		100.5021

				116.92		100.4963

				116.94		100.5021

				116.97		100.5021

				116.99		100.4963

				117.01		100.4963

				117.03		100.4963

				117.05		100.4963

				117.07		100.4963

				117.09		100.4963

				117.11		100.4963

				117.13		100.4963

				117.15		100.4963

				117.18		100.4963

				117.2		100.4963

				117.22		100.4963

				117.24		100.4963

				117.26		100.4963

				117.28		100.4963

				117.3		100.4963

				117.32		100.4963

				117.34		100.4963

				117.37		100.4906

				117.39		100.4906

				117.41		100.4906

				117.43		100.4906

				117.45		100.4906

				117.47		100.4906

				117.49		100.4906

				117.51		100.4906

				117.53		100.4906

				117.55		100.4906

				117.58		100.4906

				117.6		100.4906

				117.62		100.4906

				117.64		100.4906

				117.66		100.4906

				117.68		100.4906

				117.7		100.4906

				117.72		100.4848

				117.74		100.4848

				117.76		100.4848

				117.79		100.4848

				117.81		100.4848

				117.83		100.4848

				117.85		100.4848

				117.87		100.4848

				117.89		100.4848

				117.91		100.4848

				117.93		100.4848

				117.95		100.4848

				117.98		100.4848

				118		100.4848

				118.02		100.4848

				118.04		100.4848

				118.06		100.4848

				118.08		100.479

				118.1		100.479

				118.12		100.479

				118.14		100.479

				118.16		100.479

				118.19		100.479

				118.21		100.479

				118.23		100.479

				118.25		100.479

				118.27		100.479

				118.29		100.479

				118.31		100.479

				118.33		100.4732

				118.35		100.479

				118.37		100.4732

				118.4		100.4732

				118.42		100.4732

				118.44		100.479

				118.46		100.4732

				118.48		100.479

				118.5		100.4732

				118.52		100.4732

				118.54		100.4732

				118.56		100.4732

				118.58		100.4732

				118.61		100.4732

				118.63		100.4732

				118.65		100.4732

				118.67		100.4732

				118.69		100.4732

				118.71		100.4732

				118.73		100.4732

				118.75		100.4732

				118.77		100.4732

				118.79		100.4732

				118.82		100.4732

				118.84		100.4732

				118.86		100.4732

				118.88		100.4732

				118.9		100.4732

				118.92		100.4732

				118.94		100.4732

				118.96		100.4732

				118.98		100.4732

				119.01		100.4732

				119.03		100.4675

				119.05		100.4675

				119.07		100.4675

				119.09		100.4675

				119.11		100.4675

				119.13		100.4675

				119.15		100.4675

				119.17		100.4675

				119.19		100.4675

				119.22		100.4675

				119.24		100.4675

				119.26		100.4675

				119.28		100.4675

				119.3		100.4675

				119.32		100.4617

				119.34		100.4617

				119.36		100.4617

				119.38		100.4617

				119.4		100.4617

				119.43		100.4617

				119.45		100.4617

				119.47		100.4617

				119.49		100.4617

				119.51		100.4617

				119.53		100.4617

				119.55		100.4617

				119.57		100.4617

				119.59		100.4617

				119.61		100.4617

				119.64		100.4617

				119.66		100.4617

				119.68		100.4617

				119.7		100.4617

				119.72		100.4617

				119.74		100.4617

				119.76		100.4617

				119.78		100.4617

				119.8		100.4617

				119.82		100.4559

				119.85		100.4559

				119.87		100.4559

				119.89		100.4559

				119.91		100.4559

				119.93		100.4559

				119.95		100.4617

				119.97		100.4559

				119.99		100.4559

				120.01		100.4559

				120.03		100.4559

				120.06		100.4559

				120.08		100.4559

				120.1		100.4559

				120.12		100.4559

				120.14		100.4559

				120.16		100.4559

				120.18		100.4559

				120.2		100.4559

				120.22		100.4559

				120.24		100.4559

				120.27		100.4559

				120.29		100.4559

				120.31		100.4559

				120.33		100.4559

				120.35		100.4502

				120.37		100.4559

				120.39		100.4502

				120.41		100.4502

				120.43		100.4502

				120.45		100.4502

				120.48		100.4502

				120.5		100.4502

				120.52		100.4502

				120.54		100.4502

				120.56		100.4502

				120.58		100.4502

				120.6		100.4502

				120.62		100.4502

				120.64		100.4502

				120.67		100.4502

				120.69		100.4502

				120.71		100.4502

				120.73		100.4502

				120.75		100.4444

				120.77		100.4444

				120.79		100.4444

				120.81		100.4444

				120.83		100.4444

				120.85		100.4444

				120.88		100.4444

				120.9		100.4444

				120.92		100.4444

				120.94		100.4444

				120.96		100.4444

				120.98		100.4444

				121		100.4444

				121.02		100.4444

				121.04		100.4444

				121.06		100.4444

				121.09		100.4444

				121.11		100.4502

				121.13		100.4502

				121.15		100.4502

				121.17		100.4502

				121.19		100.4444

				121.21		100.4444

				121.23		100.4444

				121.25		100.4444

				121.27		100.4444

				121.3		100.4444

				121.32		100.4444

				121.34		100.4444

				121.36		100.4444

				121.38		100.4444

				121.4		100.4444

				121.42		100.4444

				121.44		100.4444

				121.46		100.4444

				121.48		100.4444

				121.51		100.4444

				121.53		100.4444

				121.55		100.4444

				121.57		100.4444

				121.59		100.4444

				121.61		100.4444

				121.63		100.4444

				121.65		100.4444

				121.67		100.4444

				121.7		100.4444

				121.72		100.4444

				121.74		100.4444

				121.76		100.4444

				121.78		100.4444

				121.8		100.4444

				121.82		100.4444

				121.84		100.4386

				121.86		100.4386

				121.88		100.4386

				121.91		100.4444

				121.93		100.4444

				121.95		100.4386

				121.97		100.4386

				121.99		100.4386

				122.01		100.4386

				122.03		100.4386

				122.05		100.4386

				122.07		100.4386

				122.09		100.4386

				122.12		100.4386

				122.14		100.4386

				122.16		100.4386

				122.18		100.4386

				122.2		100.4386

				122.22		100.4386

				122.24		100.4329

				122.26		100.4386

				122.28		100.4329

				122.3		100.4329

				122.33		100.4329

				122.35		100.4329

				122.37		100.4329

				122.39		100.4329

				122.41		100.4329

				122.43		100.4329

				122.45		100.4329

				122.47		100.4329

				122.49		100.4329

				122.51		100.4329

				122.54		100.4329

				122.56		100.4329

				122.58		100.4329

				122.6		100.4329

				122.62		100.4329

				122.64		100.4271

				122.66		100.4329

				122.68		100.4271

				122.7		100.4271

				122.73		100.4271

				122.75		100.4271

				122.77		100.4271

				122.79		100.4329

				122.81		100.4271

				122.83		100.4271

				122.85		100.4271

				122.87		100.4271

				122.89		100.4271

				122.91		100.4271

				122.94		100.4213

				122.96		100.4213

				122.98		100.4213

				123		100.4155

				123.02		100.4213

				123.04		100.4155

				123.06		100.4213

				123.08		100.4155

				123.1		100.4155

				123.13		100.4155

				123.15		100.4155

				123.17		100.4155

				123.19		100.4155

				123.21		100.4155

				123.23		100.4155

				123.25		100.4155

				123.27		100.4155

				123.29		100.4155

				123.31		100.4155

				123.34		100.4098

				123.36		100.4098

				123.38		100.4098

				123.4		100.4098

				123.42		100.4098

				123.44		100.4098

				123.46		100.4098

				123.48		100.4098

				123.5		100.4098

				123.53		100.4098

				123.55		100.4098

				123.57		100.4098

				123.59		100.404

				123.61		100.404

				123.63		100.404

				123.65		100.404

				123.67		100.404

				123.69		100.404

				123.71		100.404

				123.74		100.404

				123.76		100.404

				123.78		100.3982

				123.8		100.3982

				123.82		100.3982

				123.84		100.3982

				123.86		100.3982

				123.88		100.3982

				123.9		100.3982

				123.93		100.3982

				123.95		100.3982

				123.97		100.3982

				123.99		100.3982

				124.01		100.3982

				124.03		100.3982

				124.05		100.3982

				124.07		100.3982

				124.09		100.3982

				124.12		100.3982

				124.14		100.3925

				124.16		100.3982

				124.18		100.3925

				124.2		100.3925

				124.22		100.3925

				124.24		100.3925

				124.26		100.3925

				124.28		100.3925

				124.3		100.3925

				124.33		100.3925

				124.35		100.3925

				124.37		100.3925

				124.39		100.3925

				124.41		100.3925

				124.43		100.3925

				124.45		100.3925

				124.47		100.3925

				124.49		100.3867

				124.52		100.3867

				124.54		100.3867

				124.56		100.3867

				124.58		100.3867

				124.6		100.3867

				124.62		100.3867

				124.64		100.3867

				124.66		100.3867

				124.68		100.3867

				124.7		100.3867

				124.73		100.3867

				124.75		100.3867

				124.77		100.3867

				124.79		100.3867

				124.81		100.3867

				124.83		100.3867

				124.85		100.3809

				124.87		100.3809

				124.89		100.3809

				124.92		100.3809

				124.94		100.3809

				124.96		100.3809

				124.98		100.3809

				125		100.3809

				125.02		100.3809

				125.04		100.3809

				125.06		100.3809

				125.08		100.3809

				125.11		100.3809

				125.13		100.3809

				125.15		100.3809

				125.17		100.3751

				125.19		100.3809

				125.21		100.3751

				125.23		100.3809

				125.25		100.3751

				125.27		100.3751

				125.29		100.3751

				125.32		100.3809

				125.34		100.3751

				125.36		100.3751

				125.38		100.3751

				125.4		100.3751

				125.42		100.3751

				125.44		100.3751

				125.46		100.3751

				125.48		100.3751

				125.51		100.3751

				125.53		100.3751

				125.55		100.3751

				125.57		100.3751

				125.59		100.3751

				125.61		100.3751

				125.63		100.3751

				125.65		100.3694

				125.67		100.3751

				125.7		100.3751

				125.72		100.3694

				125.74		100.3694

				125.76		100.3694

				125.78		100.3694

				125.8		100.3694

				125.82		100.3694

				125.84		100.3694

				125.86		100.3694

				125.88		100.3694

				125.91		100.3694

				125.93		100.3636

				125.95		100.3636

				125.97		100.3636

				125.99		100.3636

				126.01		100.3636

				126.03		100.3636

				126.05		100.3636

				126.07		100.3636

				126.1		100.3636

				126.12		100.3636

				126.14		100.3636

				126.16		100.3636

				126.18		100.3578

				126.2		100.3578

				126.22		100.3578

				126.24		100.3578

				126.26		100.3578

				126.28		100.3578

				126.31		100.3578

				126.33		100.3578

				126.35		100.3578

				126.37		100.3578

				126.39		100.3578

				126.41		100.3521

				126.43		100.3521

				126.45		100.3521

				126.47		100.3521

				126.5		100.3521

				126.52		100.3521

				126.54		100.3521

				126.56		100.3521

				126.58		100.3521

				126.6		100.3521

				126.62		100.3521

				126.64		100.3521

				126.66		100.3521

				126.69		100.3521

				126.71		100.3521

				126.73		100.3521

				126.75		100.3463

				126.77		100.3463

				126.79		100.3463

				126.81		100.3463

				126.83		100.3463

				126.85		100.3463

				126.87		100.3463

				126.9		100.3463

				126.92		100.3463

				126.94		100.3463

				126.96		100.3463

				126.98		100.3405

				127		100.3405

				127.02		100.3405

				127.04		100.3405

				127.06		100.3405

				127.09		100.3405

				127.11		100.3405

				127.13		100.3405

				127.15		100.3405

				127.17		100.3405

				127.19		100.3405

				127.21		100.3405

				127.23		100.3405

				127.25		100.3405

				127.28		100.3405

				127.3		100.3405

				127.32		100.3347

				127.34		100.3347

				127.36		100.3347

				127.38		100.3347

				127.4		100.3347

				127.42		100.3347

				127.44		100.3347

				127.47		100.3347

				127.49		100.3347

				127.51		100.329

				127.53		100.3347

				127.55		100.3347

				127.57		100.3347

				127.59		100.3347

				127.61		100.3347

				127.63		100.3347

				127.66		100.329

				127.68		100.329

				127.7		100.329

				127.72		100.329

				127.74		100.329

				127.76		100.329

				127.78		100.329

				127.8		100.329

				127.82		100.329

				127.84		100.3232

				127.87		100.329

				127.89		100.3232

				127.91		100.3232

				127.93		100.3232

				127.95		100.3232

				127.97		100.3232

				127.99		100.3232

				128.01		100.3232

				128.03		100.3232

				128.06		100.3232

				128.08		100.3232

				128.1		100.3232

				128.12		100.3174

				128.14		100.3232

				128.16		100.3174

				128.18		100.3232

				128.2		100.3174

				128.22		100.3174

				128.25		100.3174

				128.27		100.3174

				128.29		100.3232

				128.31		100.3174

				128.33		100.3174

				128.35		100.3174

				128.37		100.3174

				128.39		100.3174

				128.41		100.3174

				128.44		100.3174

				128.46		100.3174

				128.48		100.3174

				128.5		100.3174

				128.52		100.3174

				128.54		100.3174

				128.56		100.3174

				128.58		100.3174

				128.6		100.3174

				128.63		100.3174

				128.65		100.3174

				128.67		100.3117

				128.69		100.3117

				128.71		100.3117

				128.73		100.3117

				128.75		100.3117

				128.77		100.3117

				128.79		100.3117

				128.82		100.3117

				128.84		100.3117

				128.86		100.3117

				128.88		100.3117

				128.9		100.3117

				128.92		100.3059

				128.94		100.3059

				128.96		100.3059

				128.98		100.3059

				129		100.3059

				129.03		100.3059

				129.05		100.3059

				129.07		100.3059

				129.09		100.3059

				129.11		100.3059

				129.13		100.3059

				129.15		100.3001

				129.17		100.3001

				129.19		100.3001

				129.22		100.3001

				129.24		100.3001

				129.26		100.3001

				129.28		100.3001

				129.3		100.3001

				129.32		100.3001

				129.34		100.3001

				129.36		100.3001

				129.38		100.2943

				129.41		100.2943

				129.43		100.2943

				129.45		100.2943

				129.47		100.2943

				129.49		100.2943

				129.51		100.2943

				129.53		100.2943

				129.55		100.2943

				129.57		100.2943

				129.6		100.2943

				129.62		100.2886

				129.64		100.2886

				129.66		100.2886

				129.68		100.2886

				129.7		100.2886

				129.72		100.2828

				129.74		100.2828

				129.76		100.2828

				129.79		100.2828

				129.81		100.2828

				129.83		100.2828

				129.85		100.2828

				129.87		100.2828

				129.89		100.2828

				129.91		100.2828

				129.93		100.2828

				129.95		100.2828

				129.98		100.2828

				130		100.2828

				130.02		100.277

				130.04		100.277

				130.06		100.277

				130.08		100.277

				130.1		100.277

				130.12		100.277

				130.14		100.277

				130.17		100.277

				130.19		100.2713

				130.21		100.277

				130.23		100.2655

				130.25		100.2713

				130.27		100.2713

				130.29		100.2713

				130.31		100.2655

				130.33		100.2655

				130.36		100.2655

				130.38		100.2655

				130.4		100.2655

				130.42		100.2655

				130.44		100.2597

				130.46		100.2655

				130.48		100.2655

				130.5		100.2597

				130.52		100.2597

				130.55		100.2597

				130.57		100.2597

				130.59		100.2597

				130.61		100.2597

				130.63		100.2597

				130.65		100.2597

				130.67		100.2597

				130.69		100.2597

				130.71		100.2539

				130.74		100.2539

				130.76		100.2539

				130.78		100.2539

				130.8		100.2539

				130.82		100.2539

				130.84		100.2539

				130.86		100.2482

				130.88		100.2482

				130.9		100.2482

				130.93		100.2482

				130.95		100.2482

				130.97		100.2482

				130.99		100.2482

				131.01		100.2424

				131.03		100.2424

				131.05		100.2424

				131.07		100.2424

				131.09		100.2424

				131.12		100.2424

				131.14		100.2424

				131.16		100.2424

				131.18		100.2366

				131.2		100.2366

				131.22		100.2366

				131.24		100.2366

				131.26		100.2366

				131.28		100.2366

				131.31		100.2366

				131.33		100.2366

				131.35		100.2366

				131.37		100.2366

				131.39		100.2366

				131.41		100.2366

				131.43		100.2366

				131.45		100.2366

				131.47		100.2309

				131.5		100.2309

				131.52		100.2309

				131.54		100.2309

				131.56		100.2309

				131.58		100.2309

				131.6		100.2309

				131.62		100.2309

				131.64		100.2251

				131.67		100.2251

				131.69		100.2251

				131.71		100.2251

				131.73		100.2251

				131.75		100.2251

				131.77		100.2251

				131.79		100.2251

				131.81		100.2251

				131.83		100.2251

				131.86		100.2251

				131.88		100.2193

				131.9		100.2251

				131.92		100.2193

				131.94		100.2193

				131.96		100.2193

				131.98		100.2193

				132		100.2193

				132.02		100.2193

				132.05		100.2193

				132.07		100.2193

				132.09		100.2193

				132.11		100.2135

				132.13		100.2135

				132.15		100.2135

				132.17		100.2135

				132.19		100.2135

				132.21		100.2135

				132.24		100.2135

				132.26		100.2135

				132.28		100.2135

				132.3		100.2135

				132.32		100.2135

				132.34		100.2135

				132.36		100.2135

				132.38		100.2135

				132.41		100.2135

				132.43		100.2078

				132.45		100.2135

				132.47		100.2135

				132.49		100.2078

				132.51		100.2078

				132.53		100.2078

				132.55		100.2078

				132.57		100.2078

				132.6		100.2078

				132.62		100.2078

				132.64		100.202

				132.66		100.202

				132.68		100.202

				132.7		100.202

				132.72		100.202

				132.74		100.202

				132.76		100.202

				132.79		100.202

				132.81		100.202

				132.83		100.202

				132.85		100.202

				132.87		100.1962

				132.89		100.1962

				132.91		100.1962

				132.93		100.1962

				132.96		100.1962

				132.98		100.1962

				133		100.1962

				133.02		100.1962

				133.04		100.1962

				133.06		100.1962

				133.08		100.1962

				133.1		100.1962

				133.12		100.1962

				133.15		100.1962

				133.17		100.1905

				133.19		100.1905

				133.21		100.1905

				133.23		100.1905

				133.25		100.1905

				133.27		100.1905

				133.29		100.1847

				133.31		100.1847

				133.34		100.1847

				133.36		100.1847

				133.38		100.1847

				133.4		100.1847

				133.42		100.1847

				133.44		100.1847

				133.46		100.1789

				133.48		100.1789

				133.51		100.1789

				133.53		100.1789

				133.55		100.1789

				133.57		100.1789

				133.59		100.1789

				133.61		100.1789

				133.63		100.1731

				133.65		100.1731

				133.67		100.1674

				133.7		100.1616

				133.72		100.1674

				133.74		100.1558

				133.76		100.1674

				133.78		100.1674

				133.8		100.1674

				133.82		100.1674

				133.84		100.1616

				133.86		100.1616

				133.89		100.1616

				133.91		100.1558

				133.93		100.1558

				133.95		100.1558

				133.97		100.1558

				133.99		100.1558

				134.01		100.1558

				134.03		100.1501

				134.06		100.1501

				134.08		100.1501

				134.1		100.1443

				134.12		100.1443

				134.14		100.1443

				134.16		100.1443

				134.18		100.1443

				134.2		100.1385

				134.22		100.1385

				134.25		100.1385

				134.27		100.1385

				134.29		100.1385

				134.31		100.1385

				134.33		100.1385

				134.35		100.1385

				134.37		100.1385

				134.39		100.1385

				134.41		100.1327

				134.44		100.1327

				134.46		100.1327

				134.48		100.1327

				134.5		100.1327

				134.52		100.1327

				134.54		100.1327

				134.56		100.127

				134.58		100.127

				134.61		100.127

				134.63		100.127

				134.65		100.127

				134.67		100.127

				134.69		100.127

				134.71		100.127

				134.73		100.127

				134.75		100.127

				134.77		100.127

				134.8		100.1212

				134.82		100.1212

				134.84		100.1212

				134.86		100.1212

				134.88		100.1212

				134.9		100.1212

				134.92		100.1212

				134.94		100.1154

				134.97		100.1154

				134.99		100.1154

				135.01		100.1154

				135.03		100.1154

				135.05		100.1154

				135.07		100.1154

				135.09		100.1097

				135.11		100.1097

				135.13		100.1097

				135.16		100.1097

				135.18		100.1097

				135.2		100.1097

				135.22		100.1097

				135.24		100.1097

				135.26		100.1097

				135.28		100.1097

				135.3		100.1097

				135.33		100.1039

				135.35		100.1039

				135.37		100.1097

				135.39		100.1097

				135.41		100.1039

				135.43		100.1097

				135.45		100.1097

				135.47		100.1097

				135.49		100.1039

				135.52		100.1039

				135.54		100.1039

				135.56		100.1039

				135.58		100.1039

				135.6		100.1039

				135.62		100.0981

				135.64		100.0981

				135.66		100.0981

				135.69		100.0981

				135.71		100.0981

				135.73		100.0981

				135.75		100.0981

				135.77		100.0923

				135.79		100.0923

				135.81		100.0923

				135.83		100.0923

				135.85		100.0923

				135.88		100.0866

				135.9		100.0866

				135.92		100.0866

				135.94		100.0866

				135.96		100.0866

				135.98		100.0866

				136		100.0808

				136.02		100.0866

				136.05		100.0866

				136.07		100.0808

				136.09		100.0808

				136.11		100.0808

				136.13		100.0808

				136.15		100.0808

				136.17		100.075

				136.19		100.0808

				136.21		100.075

				136.24		100.075

				136.26		100.075

				136.28		100.075

				136.3		100.075

				136.32		100.075

				136.34		100.075

				136.36		100.0693

				136.38		100.0693

				136.4		100.0693

				136.43		100.0693

				136.45		100.0693

				136.47		100.0693

				136.49		100.0693

				136.51		100.0635

				136.53		100.0693

				136.55		100.0635

				136.57		100.0635

				136.6		100.0635

				136.62		100.0635

				136.64		100.0635

				136.66		100.0635

				136.68		100.0635

				136.7		100.0635

				136.72		100.0635

				136.74		100.0635

				136.76		100.0577

				136.79		100.0577

				136.81		100.0577

				136.83		100.0577

				136.85		100.0577

				136.87		100.0577

				136.89		100.0577

				136.91		100.0577

				136.93		100.0577

				136.96		100.0519

				136.98		100.0519

				137		100.0519

				137.02		100.0519

				137.04		100.0519

				137.06		100.0519

				137.08		100.0519

				137.1		100.0462

				137.12		100.0462

				137.15		100.0462

				137.17		100.0462

				137.19		100.0462

				137.21		100.0462

				137.23		100.0462

				137.25		100.0404

				137.27		100.0462

				137.29		100.0462

				137.31		100.0462

				137.34		100.0462

				137.36		100.0462

				137.38		100.0462

				137.4		100.0462

				137.42		100.0289

				137.44		100.0115

				137.46		100.0058

				137.48		100.0058

				137.51		100

				137.53		100

				137.55		100

				137.57		99.99423

				137.59		99.99423

				137.61		99.99423

				137.63		99.99423

				137.65		99.99423

				137.67		99.98846

				137.7		99.99423

				137.72		99.98846

				137.74		99.98846

				137.76		99.98269

				137.78		99.98846

				137.8		99.99423

				137.82		99.98846

				137.84		99.99423

				137.87		99.99423

				137.89		99.99423

				137.91		99.99423

				137.93		99.99423

				137.95		100

				137.97		100

				137.99		99.99423

				138.01		99.99423

				138.03		99.99423

				138.06		99.98846

				138.08		99.98846

				138.1		99.98846

				138.12		99.98846

				138.14		99.98269

				138.16		99.98269

				138.18		99.98269

				138.2		99.97691

				138.22		99.97691

				138.25		99.97691

				138.27		99.97691

				138.29		99.97691

				138.31		99.97114

				138.33		99.97691

				138.35		99.98846

				138.37		100.0115

				138.39		100.0173

				138.42		100.0173

				138.44		100.0231

				138.46		100.0231

				138.48		100.0231

				138.5		100.0173

				138.52		100.0231

				138.54		100.0231

				138.56		100.0462

				138.58		100.0462

				138.61		100.0462

				138.63		100.0404

				138.65		100.0519

				138.67		100.0462

				138.69		100.0462

				138.71		100.0462

				138.73		100.0462

				138.75		100.0462

				138.78		100.0404

				138.8		100.0404

				138.82		100.0404

				138.84		100.0404

				138.86		100.0404

				138.88		100.0346

				138.9		100.0346

				138.92		100.0346

				138.94		100.0289

				138.97		100.0346

				138.99		100.0346

				139.01		100.0346

				139.03		100.0346

				139.05		100.0346

				139.07		100.0346

				139.09		100.0346

				139.11		100.0346

				139.14		100.0346

				139.16		100.0346

				139.18		100.0346

				139.2		100.0346

				139.22		100.0346

				139.24		100.0346

				139.26		100.0346

				139.28		100.0404

				139.31		100.0346

				139.33		100

				139.35		99.98269

				139.37		99.97114

				139.39		99.97114

				139.41		99.97114

				139.43		99.97114

				139.45		99.97114

				139.48		99.97114

				139.5		99.96537

				139.52		99.97114

				139.54		99.96537

				139.56		99.96537

				139.58		99.96537

				139.6		99.96537

				139.62		99.9596

				139.64		99.9596

				139.67		99.9596

				139.69		99.9596

				139.71		99.9596

				139.73		99.9596

				139.75		99.9596

				139.77		99.95383

				139.79		99.95383

				139.81		99.95383

				139.84		99.95383

				139.86		99.94806

				139.88		99.94806

				139.9		99.94806

				139.92		99.94229

				139.94		99.94229

				139.96		99.93652

				139.98		99.93652

				140.01		99.93652

				140.03		99.93652

				140.05		99.93074

				140.07		99.93652

				140.09		99.93652

				140.11		99.93652

				140.13		99.93074

				140.15		99.93074

				140.17		99.93074

				140.2		99.92497

				140.22		99.92497

				140.24		99.92497

				140.26		99.9192

				140.28		99.9192

				140.3		99.9192

				140.32		99.9192

				140.34		99.91343

				140.37		99.90766

				140.39		99.91343

				140.41		99.90766

				140.43		99.90766

				140.45		99.90766

				140.47		99.90766

				140.49		99.90189

				140.51		99.90189

				140.54		99.89612

				140.56		99.89612

				140.58		99.89612

				140.6		99.89612

				140.62		99.89612

				140.64		99.89034

				140.66		99.89034

				140.68		99.89034

				140.7		99.89034

				140.73		99.88457

				140.75		99.88457

				140.77		99.88457

				140.79		99.88457

				140.81		99.88457

				140.83		99.88457

				140.85		99.8788

				140.87		99.8788

				140.9		99.8788

				140.92		99.87303

				140.94		99.87303

				140.96		99.87303

				140.98		99.87303

				141		99.87303

				141.02		99.87303

				141.04		99.87303

				141.07		99.87303

				141.09		99.86726

				141.11		99.86726

				141.13		99.86726

				141.15		99.86149

				141.17		99.86149

				141.19		99.86149

				141.21		99.86149

				141.23		99.85572

				141.26		99.85572

				141.28		99.85572

				141.3		99.85572

				141.32		99.84995

				141.34		99.84995

				141.36		99.84995

				141.38		99.84995

				141.4		99.84995

				141.43		99.84995

				141.45		99.84417

				141.47		99.84417

				141.49		99.84417

				141.51		99.84417

				141.53		99.84417

				141.55		99.84417

				141.57		99.84417

				141.6		99.84417

				141.62		99.8384

				141.64		99.84417

				141.66		99.8384

				141.68		99.8384

				141.7		99.8384

				141.72		99.8384

				141.74		99.83263

				141.76		99.83263

				141.79		99.83263

				141.81		99.83263

				141.83		99.83263

				141.85		99.83263

				141.87		99.82686

				141.89		99.82686

				141.91		99.82686

				141.93		99.82686

				141.96		99.82686

				141.98		99.82109

				142		99.82686

				142.02		99.82109

				142.04		99.82109

				142.06		99.82109

				142.08		99.82109

				142.1		99.81532

				142.13		99.82109

				142.15		99.81532

				142.17		99.81532

				142.19		99.81532

				142.21		99.80955

				142.23		99.80955

				142.25		99.80955

				142.27		99.80955

				142.3		99.80377

				142.32		99.80377

				142.34		99.80377

				142.36		99.80377

				142.38		99.80377

				142.4		99.798

				142.42		99.798

				142.44		99.80377

				142.47		99.798

				142.49		99.798

				142.51		99.798

				142.53		99.798

				142.55		99.798

				142.57		99.798

				142.59		99.79223

				142.61		99.79223

				142.63		99.79223

				142.66		99.79223

				142.68		99.79223

				142.7		99.79223

				142.72		99.79223

				142.74		99.79223

				142.76		99.78646

				142.78		99.78646

				142.8		99.78646

				142.83		99.78646

				142.85		99.78069

				142.87		99.78069

				142.89		99.78069

				142.91		99.78069

				142.93		99.78069

				142.95		99.78069

				142.97		99.78069

				143		99.77492

				143.02		99.78069

				143.04		99.78069

				143.06		99.77492

				143.08		99.77492

				143.1		99.77492

				143.12		99.77492

				143.14		99.77492

				143.17		99.76915

				143.19		99.76915

				143.21		99.76338

				143.23		99.76338

				143.25		99.76338

				143.27		99.76338

				143.29		99.7576

				143.31		99.7576

				143.34		99.75183

				143.36		99.75183

				143.38		99.75183

				143.4		99.75183

				143.42		99.75183

				143.44		99.74606

				143.46		99.74606

				143.48		99.74606

				143.5		99.74606

				143.53		99.74606

				143.55		99.74606

				143.57		99.74606

				143.59		99.74606

				143.61		99.74606

				143.63		99.74029

				143.65		99.74029

				143.67		99.73452

				143.7		99.73452

				143.72		99.73452

				143.74		99.72875

				143.76		99.73452

				143.78		99.72875

				143.8		99.72875

				143.82		99.72875

				143.84		99.72298

				143.87		99.72875

				143.89		99.72298

				143.91		99.72298

				143.93		99.72298

				143.95		99.72298

				143.97		99.7172

				143.99		99.7172

				144.01		99.7172

				144.04		99.7172

				144.06		99.7172

				144.08		99.7172

				144.1		99.71143

				144.12		99.71143

				144.14		99.71143

				144.16		99.71143

				144.18		99.71143

				144.21		99.70566

				144.23		99.70566

				144.25		99.69989

				144.27		99.69989

				144.29		99.69989

				144.31		99.69412

				144.33		99.69989

				144.35		99.69412

				144.37		99.69412

				144.4		99.69412

				144.42		99.69412

				144.44		99.69412

				144.46		99.69412

				144.48		99.69412

				144.5		99.69412

				144.52		99.69412

				144.54		99.68835

				144.57		99.68835

				144.59		99.68835

				144.61		99.68835

				144.63		99.68258

				144.65		99.68258

				144.67		99.68258

				144.69		99.6768

				144.71		99.6768

				144.74		99.6768

				144.76		99.6768

				144.78		99.6768

				144.8		99.67103

				144.82		99.67103

				144.84		99.66526

				144.86		99.66526

				144.88		99.66526

				144.91		99.66526

				144.93		99.65949

				144.95		99.65949

				144.97		99.65372

				144.99		99.65372

				145.01		99.65372

				145.03		99.64795

				145.05		99.64795

				145.07		99.64795

				145.1		99.64795

				145.12		99.64218

				145.14		99.64795

				145.16		99.64218

				145.18		99.64218

				145.2		99.64218

				145.22		99.64218

				145.24		99.63641

				145.27		99.63641

				145.29		99.63641

				145.31		99.63641

				145.33		99.63063

				145.35		99.63063

				145.37		99.63063

				145.39		99.63063

				145.41		99.62486

				145.44		99.62486

				145.46		99.61909

				145.48		99.61909

				145.5		99.61909

				145.52		99.61909

				145.54		99.61332

				145.56		99.61332

				145.58		99.60755

				145.61		99.60755

				145.63		99.60178

				145.65		99.60178

				145.67		99.60178

				145.69		99.60178

				145.71		99.60178

				145.73		99.60178

				145.75		99.59601

				145.78		99.59601

				145.8		99.59601

				145.82		99.59601

				145.84		99.59601

				145.86		99.59601

				145.88		99.59023

				145.9		99.58446

				145.92		99.58446

				145.95		99.57869

				145.97		99.57292

				145.99		99.57292

				146.01		99.57292

				146.03		99.57292

				146.05		99.56138

				146.07		99.56715

				146.09		99.56138

				146.12		99.56138

				146.14		99.56138

				146.16		99.56138

				146.18		99.55561

				146.2		99.55561

				146.22		99.55561

				146.24		99.54984

				146.26		99.55561

				146.28		99.54984

				146.31		99.54984

				146.33		99.54984

				146.35		99.54406

				146.37		99.54406

				146.39		99.53829

				146.41		99.53829

				146.43		99.53829

				146.45		99.53252

				146.48		99.53252

				146.5		99.53252

				146.52		99.53252

				146.54		99.52675

				146.56		99.52675

				146.58		99.52675

				146.6		99.52675

				146.62		99.52675

				146.65		99.52675

				146.67		99.52675

				146.69		99.52675

				146.71		99.52098

				146.73		99.52098

				146.75		99.52098

				146.77		99.51521

				146.79		99.51521

				146.82		99.52098

				146.84		99.51521

				146.86		99.51521

				146.88		99.51521

				146.9		99.50944

				146.92		99.50944

				146.94		99.50944

				146.96		99.50944

				146.98		99.50944

				147.01		99.50944

				147.03		99.50944

				147.05		99.50944

				147.07		99.50944

				147.09		99.50366

				147.11		99.50366

				147.13		99.50366

				147.15		99.50366

				147.18		99.49789

				147.2		99.49789

				147.22		99.49789

				147.24		99.49789

				147.26		99.49789

				147.28		99.49789

				147.3		99.49212

				147.32		99.49212

				147.35		99.49212

				147.37		99.49212

				147.39		99.48635

				147.41		99.48635

				147.43		99.48635

				147.45		99.48635

				147.47		99.48635

				147.49		99.48635

				147.52		99.48635

				147.54		99.48635

				147.56		99.48635

				147.58		99.48635

				147.6		99.48058

				147.62		99.48058

				147.64		99.48058

				147.66		99.48058

				147.69		99.47481

				147.71		99.47481

				147.73		99.47481

				147.75		99.46904

				147.77		99.46904

				147.79		99.46904

				147.81		99.46327

				147.83		99.46327

				147.86		99.46327

				147.88		99.46327

				147.9		99.46327

				147.92		99.46327

				147.94		99.45749

				147.96		99.45749

				147.98		99.45749

				148		99.45172

				148.03		99.44595

				148.05		99.44595

				148.07		99.44595

				148.09		99.44018

				148.11		99.44018

				148.13		99.44018

				148.15		99.43441

				148.17		99.43441

				148.2		99.43441

				148.22		99.43441

				148.24		99.43441

				148.26		99.43441

				148.28		99.42864

				148.3		99.42287

				148.32		99.42287

				148.34		99.42287

				148.37		99.42287

				148.39		99.41709

				148.41		99.41709

				148.43		99.41709

				148.45		99.41709

				148.47		99.41132

				148.49		99.41132

				148.51		99.40555

				148.53		99.40555

				148.56		99.40555

				148.58		99.40555

				148.6		99.40555

				148.62		99.39978

				148.64		99.39978

				148.66		99.39978

				148.68		99.39978

				148.7		99.39401

				148.73		99.39401

				148.75		99.39401

				148.77		99.39401

				148.79		99.38824

				148.81		99.38824

				148.83		99.38824

				148.85		99.38824

				148.87		99.38247

				148.9		99.38247

				148.92		99.38247

				148.94		99.38247

				148.96		99.3767

				148.98		99.3767

				149		99.3767

				149.02		99.37092

				149.04		99.37092

				149.07		99.37092

				149.09		99.36515

				149.11		99.36515

				149.13		99.36515

				149.15		99.36515

				149.17		99.36515

				149.19		99.35938

				149.21		99.35938

				149.24		99.36515

				149.26		99.35938

				149.28		99.35361

				149.3		99.35361

				149.32		99.35361

				149.34		99.35361

				149.36		99.34784

				149.38		99.34784

				149.4		99.34784

				149.43		99.34207

				149.45		99.34207

				149.47		99.3363

				149.49		99.3363

				149.51		99.33052

				149.53		99.33052

				149.55		99.33052

				149.57		99.32475

				149.6		99.32475

				149.62		99.32475

				149.64		99.32475

				149.66		99.31898

				149.68		99.31898

				149.7		99.31898

				149.72		99.31898

				149.74		99.31898

				149.77		99.31321

				149.79		99.31321

				149.81		99.31321

				149.83		99.30744

				149.85		99.30744

				149.87		99.30167

				149.89		99.30167

				149.91		99.30167

				149.94		99.30167

				149.96		99.2959

				149.98		99.2959

				150		99.2959

				150.02		99.2959

				150.04		99.29013

				150.06		99.29013

				150.08		99.29013

				150.11		99.28435

				150.13		99.28435

				150.15		99.28435

				150.17		99.27858

				150.19		99.27281

				150.21		99.27281

				150.23		99.27281

				150.25		99.27281

				150.27		99.27281

				150.3		99.26704

				150.32		99.26704

				150.34		99.26704

				150.36		99.26704

				150.38		99.26704

				150.4		99.26127

				150.42		99.26127

				150.44		99.2555

				150.47		99.2555

				150.49		99.2555

				150.51		99.2555

				150.53		99.24973

				150.55		99.24973

				150.57		99.24973

				150.59		99.24973

				150.61		99.24395

				150.64		99.24395

				150.66		99.24395

				150.68		99.23818

				150.7		99.23241

				150.72		99.23818

				150.74		99.23241

				150.76		99.23241

				150.78		99.22664

				150.81		99.22664

				150.83		99.22087

				150.85		99.22087

				150.87		99.22087

				150.89		99.2151

				150.91		99.2151

				150.93		99.2151

				150.95		99.2151

				150.97		99.20933

				151		99.20933

				151.02		99.20356

				151.04		99.20933

				151.06		99.20356

				151.08		99.19778

				151.1		99.19778

				151.12		99.19778

				151.14		99.19201

				151.17		99.19201

				151.19		99.19201

				151.21		99.18624

				151.23		99.18624

				151.25		99.18047

				151.27		99.18047

				151.29		99.18047

				151.31		99.1747

				151.34		99.16893

				151.36		99.16893

				151.38		99.16893

				151.4		99.16316

				151.42		99.16316

				151.44		99.16316

				151.46		99.16316

				151.48		99.15738

				151.51		99.15738

				151.53		99.15738

				151.55		99.15161

				151.57		99.15161

				151.59		99.15161

				151.61		99.14584

				151.63		99.14584

				151.65		99.14007

				151.68		99.14007

				151.7		99.1343

				151.72		99.1343

				151.74		99.12853

				151.76		99.12853

				151.78		99.12276

				151.8		99.12853

				151.82		99.12276

				151.84		99.11699

				151.87		99.11699

				151.89		99.11699

				151.91		99.11699

				151.93		99.11121

				151.95		99.11121

				151.97		99.10544

				151.99		99.10544

				152.01		99.10544

				152.04		99.09967

				152.06		99.10544

				152.08		99.0939

				152.1		99.0939

				152.12		99.08813

				152.14		99.08813

				152.16		99.08236

				152.18		99.08236

				152.21		99.08236

				152.23		99.08236

				152.25		99.07659

				152.27		99.07659

				152.29		99.07659

				152.31		99.07659

				152.33		99.07081

				152.35		99.07081

				152.37		99.06504

				152.4		99.07081

				152.42		99.06504

				152.44		99.06504

				152.46		99.06504

				152.48		99.05927

				152.5		99.0535

				152.52		99.0535

				152.54		99.0535

				152.57		99.04773

				152.59		99.04773

				152.61		99.04773

				152.63		99.04196

				152.65		99.04196

				152.67		99.04196

				152.69		99.04196

				152.71		99.03619

				152.74		99.03619

				152.76		99.03619

				152.78		99.03041

				152.8		99.03041

				152.82		99.03041

				152.84		99.02464

				152.86		99.03041

				152.88		99.01887

				152.9		99.02464

				152.93		99.01887

				152.95		99.01887

				152.97		99.01887

				152.99		99.0131

				153.01		99.0131

				153.03		99.0131

				153.05		99.0131

				153.07		99.00733

				153.1		99.00733

				153.12		99.00156

				153.14		99.00156

				153.16		98.99579

				153.18		98.99579

				153.2		98.99579

				153.22		98.99579

				153.24		98.99579

				153.27		98.99002

				153.29		98.99002

				153.31		98.98424

				153.33		98.98424

				153.35		98.98424

				153.37		98.97847

				153.39		98.97847

				153.41		98.97847

				153.43		98.97847

				153.46		98.9727

				153.48		98.9727

				153.5		98.96693

				153.52		98.96693

				153.54		98.96693

				153.56		98.96693

				153.58		98.96116

				153.6		98.96116

				153.63		98.95539

				153.65		98.95539

				153.67		98.94384

				153.69		98.94384

				153.71		98.93807

				153.73		98.93807

				153.75		98.93807

				153.77		98.93807

				153.8		98.93807

				153.82		98.9323

				153.84		98.9323

				153.86		98.92653

				153.88		98.92653

				153.9		98.92076

				153.92		98.92076

				153.94		98.92076

				153.97		98.92076

				153.99		98.92076

				154.01		98.91499

				154.03		98.91499

				154.05		98.91499

				154.07		98.90345

				154.09		98.90922

				154.11		98.90345

				154.13		98.89767

				154.16		98.89767

				154.18		98.89767

				154.2		98.89767

				154.22		98.89767

				154.24		98.8919

				154.26		98.89767

				154.28		98.8919

				154.3		98.8919

				154.33		98.88613

				154.35		98.8919

				154.37		98.88613

				154.39		98.88613

				154.41		98.88036

				154.43		98.88036

				154.45		98.87459

				154.47		98.87459

				154.49		98.86882

				154.52		98.86882

				154.54		98.86882

				154.56		98.86305

				154.58		98.86305

				154.6		98.86305

				154.62		98.85727

				154.64		98.8515

				154.66		98.8515

				154.69		98.8515

				154.71		98.8515

				154.73		98.84573

				154.75		98.84573

				154.77		98.84573

				154.79		98.83996

				154.81		98.83996

				154.83		98.83419

				154.85		98.83419

				154.88		98.82842

				154.9		98.82842

				154.92		98.82265

				154.94		98.82265

				154.96		98.82265

				154.98		98.81688

				155		98.81688

				155.02		98.81688

				155.05		98.8111

				155.07		98.8111

				155.09		98.80533

				155.11		98.79956

				155.13		98.79956

				155.15		98.79379

				155.17		98.78802

				155.19		98.78802

				155.21		98.78225

				155.24		98.78225

				155.26		98.77648

				155.28		98.7707

				155.3		98.7707

				155.32		98.76493

				155.34		98.75916

				155.36		98.75916

				155.38		98.75339

				155.41		98.75339

				155.43		98.74762

				155.45		98.74762

				155.47		98.74762

				155.49		98.74762

				155.51		98.74185

				155.53		98.74185

				155.55		98.73608

				155.57		98.73608

				155.6		98.73031

				155.62		98.72453

				155.64		98.72453

				155.66		98.71299

				155.68		98.70722

				155.7		98.70145

				155.72		98.69568

				155.74		98.69568

				155.76		98.67836

				155.79		98.67836

				155.81		98.67259

				155.83		98.66682

				155.85		98.66682

				155.87		98.66105

				155.89		98.65528

				155.91		98.65528

				155.93		98.64951

				155.96		98.64374

				155.98		98.63796

				156		98.63796

				156.02		98.64374

				156.04		98.64951

				156.06		98.64374

				156.08		98.64374

				156.1		98.64374

				156.12		98.64374

				156.15		98.64374

				156.17		98.64374

				156.19		98.64374

				156.21		98.64374

				156.23		98.63796

				156.25		98.63796

				156.27		98.63796

				156.29		98.63796

				156.31		98.63219

				156.34		98.63219

				156.36		98.63219

				156.38		98.63219

				156.4		98.63219

				156.42		98.63219

				156.44		98.63219

				156.46		98.63796

				156.48		98.63219

				156.51		98.63219

				156.53		98.63219

				156.55		98.63219

				156.57		98.63219

				156.59		98.62642

				156.61		98.62642

				156.63		98.62642

				156.65		98.62642

				156.67		98.63219

				156.7		98.62642

				156.72		98.62642

				156.74		98.62642

				156.76		98.62065

				156.78		98.62065

				156.8		98.62065

				156.82		98.61488

				156.84		98.60911

				156.86		98.60911

				156.89		98.60911

				156.91		98.60334

				156.93		98.60334

				156.95		98.59756

				156.97		98.59756

				156.99		98.59756

				157.01		98.59179

				157.03		98.59179

				157.06		98.59179

				157.08		98.58602

				157.1		98.58602

				157.12		98.58025

				157.14		98.58025

				157.16		98.58025

				157.18		98.57448

				157.2		98.57448

				157.22		98.56871

				157.25		98.57448

				157.27		98.57448

				157.29		98.57448

				157.31		98.56871

				157.33		98.56871

				157.35		98.56294

				157.37		98.56294

				157.39		98.55717

				157.41		98.55717

				157.44		98.55717

				157.46		98.55139

				157.48		98.55139

				157.5		98.54562

				157.52		98.53985

				157.54		98.53408

				157.56		98.53408

				157.58		98.53408

				157.6		98.52831

				157.63		98.52831

				157.65		98.52831

				157.67		98.52254

				157.69		98.51677

				157.71		98.51677

				157.73		98.51677

				157.75		98.51099

				157.77		98.51099

				157.8		98.50522

				157.82		98.50522

				157.84		98.49945

				157.86		98.49368

				157.88		98.49368

				157.9		98.48791

				157.92		98.48214

				157.94		98.48214

				157.96		98.47637

				157.99		98.4706

				158.01		98.4706

				158.03		98.46482

				158.05		98.4706

				158.07		98.4706

				158.09		98.46482

				158.11		98.46482

				158.13		98.45328

				158.15		98.45905

				158.18		98.45328

				158.2		98.44751

				158.22		98.44751

				158.24		98.44174

				158.26		98.43597

				158.28		98.4302

				158.3		98.4302

				158.32		98.4302

				158.35		98.4302

				158.37		98.42442

				158.39		98.4302

				158.41		98.42442

				158.43		98.41865

				158.45		98.41865

				158.47		98.41865

				158.49		98.41288

				158.51		98.40711

				158.54		98.40711

				158.56		98.40134

				158.58		98.40134

				158.6		98.40134

				158.62		98.40134

				158.64		98.3898

				158.66		98.39557

				158.68		98.3898

				158.7		98.38402

				158.73		98.38402

				158.75		98.37825

				158.77		98.37825

				158.79		98.37248

				158.81		98.37248

				158.83		98.36671

				158.85		98.36094

				158.87		98.36094

				158.89		98.36094

				158.92		98.35517

				158.94		98.3494

				158.96		98.3494

				158.98		98.3494

				159		98.34363

				159.02		98.34363

				159.04		98.34363

				159.06		98.33785

				159.08		98.33208

				159.11		98.33208

				159.13		98.32631

				159.15		98.32054

				159.17		98.31477

				159.19		98.32054

				159.21		98.309

				159.23		98.31477

				159.25		98.31477

				159.27		98.31477

				159.3		98.309

				159.32		98.309

				159.34		98.30323

				159.36		98.30323

				159.38		98.29745

				159.4		98.29745

				159.42		98.29168

				159.44		98.29168

				159.46		98.29168

				159.49		98.29168

				159.51		98.28591

				159.53		98.28591

				159.55		98.28014

				159.57		98.27437

				159.59		98.27437

				159.61		98.27437

				159.63		98.2686

				159.66		98.2686

				159.68		98.26283

				159.7		98.26283

				159.72		98.26283

				159.74		98.26283

				159.76		98.25706

				159.78		98.25706

				159.8		98.25128

				159.82		98.25128

				159.85		98.24551

				159.87		98.25128

				159.89		98.24551

				159.91		98.23974

				159.93		98.24551

				159.95		98.23974

				159.97		98.23974

				159.99		98.23974

				160.01		98.23397

				160.04		98.2282

				160.06		98.22243

				160.08		98.22243

				160.1		98.22243

				160.12		98.21666

				160.14		98.21088

				160.16		98.21666

				160.18		98.21666

				160.2		98.21088

				160.23		98.20511

				160.25		98.20511

				160.27		98.20511

				160.29		98.20511

				160.31		98.19934

				160.33		98.19934

				160.35		98.19934

				160.37		98.19357

				160.39		98.1878

				160.42		98.1878

				160.44		98.18203

				160.46		98.18203

				160.48		98.17626

				160.5		98.17626

				160.52		98.17049

				160.54		98.17049

				160.56		98.17049

				160.58		98.16471

				160.61		98.15894

				160.63		98.15894

				160.65		98.15317

				160.67		98.15317

				160.69		98.15317

				160.71		98.1474

				160.73		98.14163

				160.75		98.14163

				160.77		98.13586

				160.8		98.13009

				160.82		98.13586

				160.84		98.13009

				160.86		98.13009

				160.88		98.12431

				160.9		98.12431

				160.92		98.12431

				160.94		98.11854

				160.96		98.11854

				160.99		98.11277

				161.01		98.11277

				161.03		98.10123

				161.05		98.107

				161.07		98.10123

				161.09		98.08969

				161.11		98.09546

				161.13		98.09546

				161.15		98.08392

				161.18		98.07814

				161.2		98.08392

				161.22		98.07814

				161.24		98.07237

				161.26		98.07237

				161.28		98.07237

				161.3		98.0666

				161.32		98.0666

				161.34		98.06083

				161.37		98.0666

				161.39		98.05506

				161.41		98.06083

				161.43		98.04929

				161.45		98.04352

				161.47		98.04352

				161.49		98.04352

				161.51		98.03774

				161.53		98.03774

				161.56		98.03774

				161.58		98.03774

				161.6		98.03197

				161.62		98.03197

				161.64		98.0262

				161.66		98.0262

				161.68		98.0262

				161.7		98.03197

				161.72		98.0262

				161.75		98.02043

				161.77		98.02043

				161.79		98.02043

				161.81		98.01466

				161.83		98.00889

				161.85		98.00889

				161.87		98.00312

				161.89		97.99735

				161.91		97.99735

				161.94		97.99157

				161.96		97.9858

				161.98		97.99157

				162		97.9858

				162.02		97.98003

				162.04		97.97426

				162.06		97.98003

				162.08		97.97426

				162.1		97.96849

				162.13		97.96272

				162.15		97.96272

				162.17		97.95695

				162.19		97.95695

				162.21		97.95117

				162.23		97.9454

				162.25		97.9454

				162.27		97.9454

				162.29		97.93963

				162.31		97.93386

				162.34		97.93963

				162.36		97.93386

				162.38		97.92809

				162.4		97.92809

				162.42		97.92809

				162.44		97.92809

				162.46		97.92232

				162.48		97.92232

				162.5		97.91655

				162.53		97.91078

				162.55		97.91078

				162.57		97.91078

				162.59		97.905

				162.61		97.905

				162.63		97.89923

				162.65		97.905

				162.67		97.89923

				162.69		97.89923

				162.72		97.89346

				162.74		97.89346

				162.76		97.88769

				162.78		97.88769

				162.8		97.88769

				162.82		97.88192

				162.84		97.88769

				162.86		97.87615

				162.88		97.87615

				162.91		97.87615

				162.93		97.87038

				162.95		97.8646

				162.97		97.8646

				162.99		97.85883

				163.01		97.85883

				163.03		97.85306

				163.05		97.85306

				163.07		97.85306

				163.1		97.84729

				163.12		97.84729

				163.14		97.84152

				163.16		97.84152

				163.18		97.84152

				163.2		97.82998

				163.22		97.82998

				163.24		97.8242

				163.26		97.81843

				163.29		97.81266

				163.31		97.81266

				163.33		97.80689

				163.35		97.80112

				163.37		97.80112

				163.39		97.79535

				163.41		97.79535

				163.43		97.79535

				163.45		97.78958

				163.48		97.78958

				163.5		97.78381

				163.52		97.78381

				163.54		97.78381

				163.56		97.77803

				163.58		97.77226

				163.6		97.77226

				163.62		97.76649

				163.64		97.76072

				163.67		97.76649

				163.69		97.76072

				163.71		97.76072

				163.73		97.75495

				163.75		97.74918

				163.77		97.74918

				163.79		97.74341

				163.81		97.73763

				163.83		97.73763

				163.85		97.73186

				163.88		97.72609

				163.9		97.72609

				163.92		97.72032

				163.94		97.71455

				163.96		97.71455

				163.98		97.70878

				164		97.70878

				164.02		97.69724

				164.04		97.69724

				164.07		97.69146

				164.09		97.68569

				164.11		97.68569

				164.13		97.67415

				164.15		97.67415

				164.17		97.66838

				164.19		97.66838

				164.21		97.66838

				164.23		97.66838

				164.26		97.66261

				164.28		97.66261

				164.3		97.65684

				164.32		97.65684

				164.34		97.65106

				164.36		97.65106

				164.38		97.64529

				164.4		97.63952

				164.42		97.63952

				164.45		97.63952

				164.47		97.63952

				164.49		97.62798

				164.51		97.63375

				164.53		97.62798

				164.55		97.62798

				164.57		97.62798

				164.59		97.62221

				164.61		97.61644

				164.63		97.62221

				164.66		97.61644

				164.68		97.61644

				164.7		97.61067

				164.72		97.61067

				164.74		97.61067

				164.76		97.60489

				164.78		97.60489

				164.8		97.60489

				164.82		97.59912

				164.85		97.59912

				164.87		97.59335

				164.89		97.59335

				164.91		97.58758

				164.93		97.58758

				164.95		97.58181

				164.97		97.58181

				164.99		97.57604

				165.01		97.57604

				165.03		97.57027

				165.06		97.57604

				165.08		97.57027

				165.1		97.57027

				165.12		97.56449

				165.14		97.56449

				165.16		97.55872

				165.18		97.55872

				165.2		97.55295

				165.22		97.55295

				165.25		97.55295

				165.27		97.54718

				165.29		97.54718

				165.31		97.54141

				165.33		97.54141

				165.35		97.52987

				165.37		97.52987

				165.39		97.52987

				165.41		97.5241

				165.44		97.51832

				165.46		97.51832

				165.48		97.51255

				165.5		97.50678

				165.52		97.50678

				165.54		97.50101

				165.56		97.49524

				165.58		97.48947

				165.6		97.48947

				165.62		97.48947

				165.65		97.4837

				165.67		97.4837

				165.69		97.47792

				165.71		97.47215

				165.73		97.47215

				165.75		97.46638

				165.77		97.46638

				165.79		97.46061

				165.81		97.46061

				165.84		97.45484

				165.86		97.44907

				165.88		97.44907

				165.9		97.44907

				165.92		97.44907

				165.94		97.4433

				165.96		97.43753

				165.98		97.43753

				166		97.42598

				166.02		97.42598

				166.05		97.42598

				166.07		97.41444

				166.09		97.40867

				166.11		97.40867

				166.13		97.4029

				166.15		97.39713

				166.17		97.39713

				166.19		97.39713

				166.21		97.39713

				166.24		97.39135

				166.26		97.37981

				166.28		97.37981

				166.3		97.38558

				166.32		97.37981

				166.34		97.37404

				166.36		97.37404

				166.38		97.36827

				166.4		97.36827

				166.43		97.3625

				166.45		97.35673

				166.47		97.3625

				166.49		97.35673

				166.51		97.35673

				166.53		97.35096

				166.55		97.34518

				166.57		97.34518

				166.59		97.33941

				166.61		97.34518

				166.64		97.33941

				166.66		97.33941

				166.68		97.33364

				166.7		97.33364

				166.72		97.32787

				166.74		97.3221

				166.76		97.32787

				166.78		97.31633

				166.8		97.31633

				166.82		97.31056

				166.85		97.31633

				166.87		97.31056

				166.89		97.31056

				166.91		97.30478

				166.93		97.31056

				166.95		97.30478

				166.97		97.30478

				166.99		97.29901

				167.01		97.29901

				167.04		97.29901

				167.06		97.29901

				167.08		97.28747

				167.1		97.28747

				167.12		97.28747

				167.14		97.28747

				167.16		97.27593

				167.18		97.27593

				167.2		97.27016

				167.22		97.27016

				167.25		97.26439

				167.27		97.25861

				167.29		97.25861

				167.31		97.25861

				167.33		97.25284

				167.35		97.2413

				167.37		97.2413

				167.39		97.2413

				167.41		97.22976

				167.44		97.22976

				167.46		97.22399

				167.48		97.22976

				167.5		97.21821

				167.52		97.22399

				167.54		97.21244

				167.56		97.21244

				167.58		97.20667

				167.6		97.20667

				167.62		97.2009

				167.65		97.2009

				167.67		97.19513

				167.69		97.19513

				167.71		97.18936

				167.73		97.18936

				167.75		97.18936

				167.77		97.18936

				167.79		97.18936

				167.81		97.17781

				167.83		97.17781

				167.86		97.17204

				167.88		97.16627

				167.9		97.1605

				167.92		97.1605

				167.94		97.14896

				167.96		97.14896

				167.98		97.14319

				168		97.14319

				168.02		97.13742

				168.05		97.13164

				168.07		97.13164

				168.09		97.1201

				168.11		97.1201

				168.13		97.12587

				168.15		97.11433

				168.17		97.10856

				168.19		97.10279

				168.21		97.10279

				168.23		97.09702

				168.26		97.09124

				168.28		97.08547

				168.3		97.08547

				168.32		97.07393

				168.34		97.07393

				168.36		97.06816

				168.38		97.06816

				168.4		97.05662

				168.42		97.06239

				168.44		97.05662

				168.47		97.05662

				168.49		97.05662

				168.51		97.05085

				168.53		97.05085

				168.55		97.04507

				168.57		97.0393

				168.59		97.0393

				168.61		97.03353

				168.63		97.03353

				168.65		97.03353

				168.68		97.02776

				168.7		97.02776

				168.72		97.02776

				168.74		97.01622

				168.76		97.01622

				168.78		97.01045

				168.8		97.00467

				168.82		96.9989

				168.84		96.9989

				168.87		96.99313

				168.89		96.98736

				168.91		96.97582

				168.93		96.97582

				168.95		96.97582

				168.97		96.97005

				168.99		96.96428

				169.01		96.9585

				169.03		96.9585

				169.05		96.95273

				169.08		96.95273

				169.1		96.95273

				169.12		96.95273

				169.14		96.94696

				169.16		96.94119

				169.18		96.94119

				169.2		96.93542

				169.22		96.93542

				169.24		96.93542

				169.26		96.92965

				169.29		96.92965

				169.31		96.93542

				169.33		96.92965

				169.35		96.92965

				169.37		96.92965

				169.39		96.92388

				169.41		96.92388

				169.43		96.9181

				169.45		96.9181

				169.47		96.90656

				169.5		96.90656

				169.52		96.90079

				169.54		96.89502

				169.56		96.90079

				169.58		96.88925

				169.6		96.88348

				169.62		96.88348

				169.64		96.88348

				169.66		96.87193

				169.68		96.86616

				169.71		96.86616

				169.73		96.86039

				169.75		96.85462

				169.77		96.85462

				169.79		96.84885

				169.81		96.84308

				169.83		96.83731

				169.85		96.84308

				169.87		96.83731

				169.9		96.83731

				169.92		96.83153

				169.94		96.82576

				169.96		96.81999

				169.98		96.82576

				170		96.81999

				170.02		96.81422

				170.04		96.80845

				170.06		96.81422

				170.08		96.80268

				170.11		96.79691

				170.13		96.79691

				170.15		96.79114

				170.17		96.78536

				170.19		96.77959

				170.21		96.77959

				170.23		96.76805

				170.25		96.76228

				170.27		96.75651

				170.29		96.75651

				170.32		96.75074

				170.34		96.75074

				170.36		96.75074

				170.38		96.73919

				170.4		96.73919

				170.42		96.74496

				170.44		96.73919

				170.46		96.73342

				170.48		96.72765

				170.5		96.73919

				170.53		96.72765

				170.55		96.72765

				170.57		96.72765

				170.59		96.72188

				170.61		96.71034

				170.63		96.71034

				170.65		96.71611

				170.67		96.69879

				170.69		96.69879

				170.71		96.69879

				170.74		96.69302

				170.76		96.68725

				170.78		96.69302

				170.8		96.68725

				170.82		96.67571

				170.84		96.67571

				170.86		96.66994

				170.88		96.66417

				170.9		96.65839

				170.92		96.65839

				170.95		96.65262

				170.97		96.64685

				170.99		96.64685

				171.01		96.64108

				171.03		96.63531

				171.05		96.62954

				171.07		96.62954

				171.09		96.62377

				171.11		96.61222

				171.14		96.61222

				171.16		96.60645

				171.18		96.60068

				171.2		96.60068

				171.22		96.59491

				171.24		96.58914

				171.26		96.59491

				171.28		96.58914

				171.3		96.58337

				171.32		96.58337

				171.35		96.57182

				171.37		96.5776

				171.39		96.57182

				171.41		96.57182

				171.43		96.57182

				171.45		96.56605

				171.47		96.56605

				171.49		96.56605

				171.51		96.56028

				171.53		96.55451

				171.56		96.55451

				171.58		96.55451

				171.6		96.54297

				171.62		96.5372

				171.64		96.54297

				171.66		96.52565

				171.68		96.52565

				171.7		96.52565

				171.72		96.51988

				171.74		96.51411

				171.77		96.50834

				171.79		96.51411

				171.81		96.50834

				171.83		96.4968

				171.85		96.50257

				171.87		96.50257

				171.89		96.4968

				171.91		96.4968

				171.93		96.4968

				171.95		96.48525

				171.98		96.48525

				172		96.47948

				172.02		96.47371

				172.04		96.47371

				172.06		96.46794

				172.08		96.46794

				172.1		96.4564

				172.12		96.46217

				172.14		96.44485

				172.16		96.43908

				172.19		96.43331

				172.21		96.43908

				172.23		96.416

				172.25		96.416

				172.27		96.41023

				172.29		96.41023

				172.31		96.41023

				172.33		96.41023

				172.35		96.41023

				172.37		96.39868

				172.4		96.39291

				172.42		96.39291

				172.44		96.38714

				172.46		96.38714

				172.48		96.38137

				172.5		96.38714

				172.52		96.3756

				172.54		96.3756

				172.56		96.36406

				172.58		96.36983

				172.61		96.36406

				172.63		96.35251

				172.65		96.34674

				172.67		96.34097

				172.69		96.3352

				172.71		96.3352

				172.73		96.32943

				172.75		96.32943

				172.77		96.32943

				172.79		96.32366

				172.82		96.31789

				172.84		96.31211

				172.86		96.31211

				172.88		96.30634

				172.9		96.30634

				172.92		96.30634

				172.94		96.30634

				172.96		96.30057

				172.98		96.30057

				173		96.2948

				173.03		96.28903

				173.05		96.28326

				173.07		96.27749

				173.09		96.27749

				173.11		96.27171

				173.13		96.27171

				173.15		96.26017

				173.17		96.26594

				173.19		96.2544

				173.21		96.2544

				173.24		96.24863

				173.26		96.24286

				173.28		96.23709

				173.3		96.23709

				173.32		96.23132

				173.34		96.22554

				173.36		96.21977

				173.38		96.214

				173.4		96.214

				173.42		96.214

				173.45		96.20823

				173.47		96.20823

				173.49		96.20246

				173.51		96.20246

				173.53		96.19669

				173.55		96.19669

				173.57		96.19669

				173.59		96.19092

				173.61		96.18514

				173.63		96.18514

				173.66		96.1736

				173.68		96.1736

				173.7		96.16783

				173.72		96.16206

				173.74		96.15629

				173.76		96.15629

				173.78		96.15629

				173.8		96.15052

				173.82		96.14475

				173.84		96.14475

				173.87		96.1332

				173.89		96.1332

				173.91		96.1332

				173.93		96.12743

				173.95		96.11589

				173.97		96.11589

				173.99		96.11012

				174.01		96.10435

				174.03		96.09857

				174.05		96.0928

				174.08		96.08703

				174.1		96.08126

				174.12		96.07549

				174.14		96.06395

				174.16		96.05818

				174.18		96.05818

				174.2		96.04663

				174.22		96.0524

				174.24		96.04663

				174.26		96.04086

				174.29		96.04086

				174.31		96.04086

				174.33		96.03509

				174.35		96.02932

				174.37		96.02355

				174.39		96.02932

				174.41		96.01778

				174.43		96.01778

				174.45		96.02355

				174.47		96.01778

				174.5		96.02355

				174.52		96.01778

				174.54		96.012

				174.56		96.012

				174.58		96.00046

				174.6		96.00046

				174.62		95.98892

				174.64		95.98315

				174.66		95.97738

				174.68		95.97161

				174.71		95.96583

				174.73		95.96583

				174.75		95.96006

				174.77		95.96006

				174.79		95.96006

				174.81		95.94852

				174.83		95.94852

				174.85		95.94275

				174.87		95.93121

				174.89		95.93121

				174.92		95.93121

				174.94		95.91966

				174.96		95.92543

				174.98		95.92543

				175		95.91389

				175.02		95.91389

				175.04		95.90812

				175.06		95.90812

				175.08		95.90235

				175.1		95.89658

				175.13		95.89658

				175.15		95.89081

				175.17		95.89081

				175.19		95.88503

				175.21		95.87926

				175.23		95.87926

				175.25		95.86772

				175.27		95.86772

				175.29		95.86195

				175.31		95.85618

				175.34		95.85041

				175.36		95.84464

				175.38		95.84464

				175.4		95.84464

				175.42		95.83886

				175.44		95.83309

				175.46		95.83309

				175.48		95.82155

				175.5		95.81578

				175.52		95.81001

				175.55		95.81001

				175.57		95.79846

				175.59		95.79846

				175.61		95.79269

				175.63		95.79269

				175.65		95.78692

				175.67		95.78115

				175.69		95.77538

				175.71		95.76384

				175.73		95.76384

				175.76		95.75807

				175.78		95.75229

				175.8		95.75229

				175.82		95.75229

				175.84		95.74075

				175.86		95.74075

				175.88		95.73498

				175.9		95.72921

				175.92		95.72921

				175.94		95.72344

				175.97		95.71767

				175.99		95.71767

				176.01		95.71189

				176.03		95.70612

				176.05		95.70612

				176.07		95.69458

				176.09		95.68881

				176.11		95.68881

				176.13		95.67727

				176.15		95.67727

				176.18		95.6715

				176.2		95.66572

				176.22		95.65995

				176.24		95.64841

				176.26		95.64841

				176.28		95.64264

				176.3		95.6311

				176.32		95.62532

				176.34		95.6311

				176.36		95.62532

				176.38		95.61955

				176.41		95.60801

				176.43		95.60801

				176.45		95.60224

				176.47		95.60224

				176.49		95.59647

				176.51		95.5907

				176.53		95.5907

				176.55		95.5907

				176.57		95.5907

				176.59		95.58493

				176.62		95.58493

				176.64		95.57338

				176.66		95.57338

				176.68		95.56761

				176.7		95.56184

				176.72		95.55607

				176.74		95.55607

				176.76		95.54453

				176.78		95.54453

				176.8		95.54453

				176.83		95.53298

				176.85		95.53298

				176.87		95.52721

				176.89		95.52721

				176.91		95.51567

				176.93		95.52144

				176.95		95.5099

				176.97		95.50413

				176.99		95.5099

				177.01		95.50413

				177.04		95.50413

				177.06		95.49836

				177.08		95.49836

				177.1		95.49258

				177.12		95.49258

				177.14		95.49258

				177.16		95.48104

				177.18		95.48104

				177.2		95.47527

				177.22		95.47527

				177.25		95.4695

				177.27		95.46373

				177.29		95.45796

				177.31		95.45796

				177.33		95.45218

				177.35		95.44641

				177.37		95.44641

				177.39		95.44064

				177.41		95.43487

				177.43		95.42333

				177.46		95.42333

				177.48		95.41756

				177.5		95.41179

				177.52		95.40601

				177.54		95.40024

				177.56		95.40024

				177.58		95.39447

				177.6		95.39447

				177.62		95.39447

				177.64		95.39447

				177.67		95.37716

				177.69		95.38293

				177.71		95.37139

				177.73		95.35984

				177.75		95.36561

				177.77		95.35984

				177.79		95.35984

				177.81		95.35407

				177.83		95.3483

				177.85		95.34253

				177.88		95.33676

				177.9		95.33099

				177.92		95.31944

				177.94		95.31944

				177.96		95.31367

				177.98		95.3079

				178		95.3079

				178.02		95.29636

				178.04		95.29059

				178.06		95.30213

				178.08		95.29636

				178.11		95.28482

				178.13		95.27904

				178.15		95.27904

				178.17		95.27327

				178.19		95.2675

				178.21		95.27327

				178.23		95.2675

				178.25		95.25596

				178.27		95.25596

				178.29		95.25019

				178.32		95.25019

				178.34		95.25019

				178.36		95.24442

				178.38		95.24442

				178.4		95.2271

				178.42		95.23287

				178.44		95.23287

				178.46		95.2271

				178.48		95.22133

				178.5		95.22133

				178.52		95.21556

				178.55		95.20979

				178.57		95.20402

				178.59		95.19825

				178.61		95.19247

				178.63		95.1867

				178.65		95.18093

				178.67		95.17516

				178.69		95.16939

				178.71		95.16362

				178.73		95.16362

				178.76		95.15207

				178.78		95.1463

				178.8		95.14053

				178.82		95.13476

				178.84		95.13476

				178.86		95.12899

				178.88		95.12322

				178.9		95.12322

				178.92		95.12322

				178.94		95.12322

				178.97		95.12322

				178.99		95.12322

				179.01		95.11745

				179.03		95.11745

				179.05		95.1059

				179.07		95.1059

				179.09		95.1059

				179.11		95.10013

				179.13		95.09436

				179.15		95.08859

				179.17		95.07705

				179.2		95.07705

				179.22		95.05973

				179.24		95.05396

				179.26		95.04819

				179.28		95.03665

				179.3		95.02511

				179.32		95.02511

				179.34		95.01356

				179.36		95.00202

				179.38		95.00779

				179.41		94.99625

				179.43		94.99048

				179.45		94.98471

				179.47		94.97893

				179.49		94.97893

				179.51		94.97316

				179.53		94.96739

				179.55		94.96739

				179.57		94.96162

				179.59		94.95585

				179.61		94.95585

				179.64		94.95585

				179.66		94.93854

				179.68		94.93854

				179.7		94.93854

				179.72		94.93276

				179.74		94.93276

				179.76		94.92699

				179.78		94.92699

				179.8		94.91545

				179.82		94.90968

				179.85		94.91545

				179.87		94.90968

				179.89		94.89236

				179.91		94.89814

				179.93		94.89236

				179.95		94.88082

				179.97		94.87505

				179.99		94.87505

				180.01		94.86351

				180.03		94.86351

				180.06		94.84619

				180.08		94.85197

				180.1		94.84619

				180.12		94.84042

				180.14		94.83465

				180.16		94.83465

				180.18		94.82311

				180.2		94.82888

				180.22		94.82888

				180.24		94.81734

				180.27		94.81157

				180.29		94.80579

				180.31		94.79425

				180.33		94.79425

				180.35		94.78271

				180.37		94.78271

				180.39		94.77117

				180.41		94.7654

				180.43		94.7654

				180.45		94.75962

				180.47		94.74231

				180.5		94.74231

				180.52		94.73654

				180.54		94.725

				180.56		94.725

				180.58		94.725

				180.6		94.71922

				180.62		94.71345

				180.64		94.70768

				180.66		94.70191

				180.68		94.70191

				180.71		94.70191

				180.73		94.69037

				180.75		94.6846

				180.77		94.67882

				180.79		94.67305

				180.81		94.67305

				180.83		94.65574

				180.85		94.64997

				180.87		94.64997

				180.89		94.6442

				180.92		94.63843

				180.94		94.63843

				180.96		94.63265

				180.98		94.62111

				181		94.62111

				181.02		94.62111

				181.04		94.60957

				181.06		94.6038

				181.08		94.6038

				181.1		94.6038

				181.13		94.59803

				181.15		94.59225

				181.17		94.58648

				181.19		94.57494

				181.21		94.57494

				181.23		94.5634

				181.25		94.5634

				181.27		94.55763

				181.29		94.55763

				181.31		94.54608

				181.34		94.54608

				181.36		94.54031

				181.38		94.53454

				181.4		94.523

				181.42		94.523

				181.44		94.523

				181.46		94.50568

				181.48		94.51146

				181.5		94.50568

				181.52		94.50568

				181.54		94.49991

				181.57		94.48837

				181.59		94.49414

				181.61		94.4826

				181.63		94.47683

				181.65		94.47106

				181.67		94.45951

				181.69		94.44797

				181.71		94.45374

				181.73		94.45374

				181.75		94.43643

				181.78		94.43643

				181.8		94.43066

				181.82		94.41911

				181.84		94.41334

				181.86		94.40757

				181.88		94.40757

				181.9		94.4018

				181.92		94.39603

				181.94		94.39026

				181.96		94.39603

				181.99		94.39603

				182.01		94.38449

				182.03		94.37872

				182.05		94.37872

				182.07		94.37294

				182.09		94.36717

				182.11		94.37294

				182.13		94.36717

				182.15		94.35563

				182.17		94.35563

				182.19		94.35563

				182.22		94.34409

				182.24		94.33832

				182.26		94.33254

				182.28		94.32677

				182.3		94.321

				182.32		94.31523

				182.34		94.31523

				182.36		94.30946

				182.38		94.29792

				182.4		94.29215

				182.43		94.28637

				182.45		94.2806

				182.47		94.28637

				182.49		94.26906

				182.51		94.25752

				182.53		94.26906

				182.55		94.26906

				182.57		94.26329

				182.59		94.25752

				182.61		94.25175

				182.63		94.24597

				182.66		94.2402

				182.68		94.22866

				182.7		94.23443

				182.72		94.22866

				182.74		94.22866

				182.76		94.22289

				182.78		94.21712

				182.8		94.21135

				182.82		94.22289

				182.84		94.21135

				182.86		94.1998

				182.89		94.1998

				182.91		94.1998

				182.93		94.19403

				182.95		94.19403

				182.97		94.19403

				182.99		94.19403

				183.01		94.18826

				183.03		94.18249

				183.05		94.17672

				183.07		94.16518

				183.1		94.16518

				183.12		94.16518

				183.14		94.15363

				183.16		94.14209

				183.18		94.14209

				183.2		94.13632

				183.22		94.13055

				183.24		94.12478

				183.26		94.12478

				183.28		94.11323

				183.3		94.10746

				183.33		94.10746

				183.35		94.10169

				183.37		94.09592

				183.39		94.10169

				183.41		94.09592

				183.43		94.08438

				183.45		94.08438

				183.47		94.08438

				183.49		94.07283

				183.51		94.07283

				183.53		94.06706

				183.56		94.06129

				183.58		94.04975

				183.6		94.04975

				183.62		94.04975

				183.64		94.03243

				183.66		94.03243

				183.68		94.03243

				183.7		94.02089

				183.72		94.00935

				183.74		94.01512

				183.77		94.00358

				183.79		93.99781

				183.81		93.99781

				183.83		93.99204

				183.85		93.98049

				183.87		93.98049

				183.89		93.98049

				183.91		93.97472

				183.93		93.97472

				183.95		93.96895

				183.97		93.95741

				184		93.96318

				184.02		93.96318

				184.04		93.94586

				184.06		93.94586

				184.08		93.95164

				184.1		93.94009

				184.12		93.94009

				184.14		93.94586

				184.16		93.92278

				184.18		93.91701

				184.2		93.91701

				184.23		93.90547

				184.25		93.89392

				184.27		93.88815

				184.29		93.88815

				184.31		93.88238

				184.33		93.87084

				184.35		93.86507

				184.37		93.86507

				184.39		93.85352

				184.41		93.85352

				184.43		93.85352

				184.46		93.84775

				184.48		93.85352

				184.5		93.85352

				184.52		93.84198

				184.54		93.83621

				184.56		93.83621

				184.58		93.83044

				184.6		93.82467

				184.62		93.82467

				184.64		93.81312

				184.67		93.80735

				184.69		93.79004

				184.71		93.79581

				184.73		93.78427

				184.75		93.76695

				184.77		93.76118

				184.79		93.75541

				184.81		93.74964

				184.83		93.74964

				184.85		93.74387

				184.87		93.7381

				184.9		93.74387

				184.92		93.7381

				184.94		93.73233

				184.96		93.73233

				184.98		93.73233

				185		93.73233

				185.02		93.72655

				185.04		93.72655

				185.06		93.72655

				185.08		93.71501

				185.11		93.70924

				185.13		93.72078

				185.15		93.70924

				185.17		93.70347

				185.19		93.69193

				185.21		93.69193

				185.23		93.68038

				185.25		93.68038

				185.27		93.67461

				185.29		93.66307

				185.31		93.64576

				185.34		93.64576

				185.36		93.65153

				185.38		93.63998

				185.4		93.62844

				185.42		93.63421

				185.44		93.62844

				185.46		93.62267

				185.48		93.62267

				185.5		93.62267

				185.52		93.60536

				185.55		93.59381

				185.57		93.61113

				185.59		93.60536

				185.61		93.58804

				185.63		93.58227

				185.65		93.5765

				185.67		93.56496

				185.69		93.55919

				185.71		93.56496

				185.73		93.54187

				185.75		93.53033

				185.78		93.53033

				185.8		93.53033

				185.82		93.52456

				185.84		93.51301

				185.86		93.51301

				185.88		93.51301

				185.9		93.50147

				185.92		93.50724

				185.94		93.4957

				185.96		93.4957

				185.98		93.48993

				186.01		93.50147

				186.03		93.4957

				186.05		93.48993

				186.07		93.48993

				186.09		93.48416

				186.11		93.47839

				186.13		93.47261

				186.15		93.46684

				186.17		93.46107

				186.19		93.4553

				186.22		93.4553

				186.24		93.44376

				186.26		93.43222

				186.28		93.42644

				186.3		93.42644

				186.32		93.40913

				186.34		93.40336

				186.36		93.40913

				186.38		93.39759

				186.4		93.40336

				186.42		93.39759

				186.45		93.39759

				186.47		93.39182

				186.49		93.39182

				186.51		93.39182

				186.53		93.38604

				186.55		93.38604

				186.57		93.3745

				186.59		93.36873

				186.61		93.36296

				186.63		93.36296

				186.65		93.35719

				186.68		93.33987

				186.7		93.3341

				186.72		93.32833

				186.74		93.31102

				186.76		93.30525

				186.78		93.30525

				186.8		93.2937

				186.82		93.28216

				186.84		93.28216

				186.86		93.28216

				186.88		93.27639

				186.91		93.26485

				186.93		93.27062

				186.95		93.27062

				186.97		93.25908

				186.99		93.27062

				187.01		93.26485

				187.03		93.25908

				187.05		93.25908

				187.07		93.25908

				187.09		93.24176

				187.12		93.24176

				187.14		93.23599

				187.16		93.23022

				187.18		93.21868

				187.2		93.20136

				187.22		93.19559

				187.24		93.19559

				187.26		93.18405

				187.28		93.18982

				187.3		93.17828

				187.32		93.17251

				187.35		93.16673

				187.37		93.16673

				187.39		93.15519

				187.41		93.15519

				187.43		93.15519

				187.45		93.14942

				187.47		93.14942

				187.49		93.14942

				187.51		93.13788

				187.53		93.13211

				187.55		93.12633

				187.57		93.12633

				187.6		93.11479

				187.62		93.10902

				187.64		93.09748

				187.66		93.09171

				187.68		93.08016

				187.7		93.08016

				187.72		93.07439

				187.74		93.06285

				187.76		93.05708

				187.78		93.05708

				187.81		93.04554

				187.83		93.03399

				187.85		93.02822

				187.87		93.02245

				187.89		93.02245

				187.91		93.02822

				187.93		93.02245

				187.95		93.01668

				187.97		93.00514

				187.99		93.01091

				188.01		93.00514

				188.04		92.99937

				188.06		93.00514

				188.08		92.99359

				188.1		92.98205

				188.12		92.98205

				188.14		92.97051

				188.16		92.96474

				188.18		92.95319

				188.2		92.94742

				188.22		92.93588

				188.24		92.93011

				188.27		92.91857

				188.29		92.91857

				188.31		92.91857

				188.33		92.87817

				188.35		92.87817

				188.37		92.8724

				188.39		92.8724

				188.41		92.8724

				188.43		92.8724

				188.45		92.8724

				188.47		92.86085

				188.5		92.86662

				188.52		92.85508

				188.54		92.84931

				188.56		92.84354

				188.58		92.832

				188.6		92.84354

				188.62		92.84931

				188.64		92.84354

				188.66		92.82622

				188.68		92.82045

				188.7		92.81468

				188.73		92.80314

				188.75		92.80314

				188.77		92.79737

				188.79		92.79737

				188.81		92.7916

				188.83		92.7916

				188.85		92.78583

				188.87		92.78005

				188.89		92.77428

				188.91		92.77428

				188.93		92.76851

				188.96		92.76851

				188.98		92.76851

				189		92.75697

				189.02		92.7512

				189.04		92.7512

				189.06		92.7512

				189.08		92.73965

				189.1		92.72811

				189.12		92.72811

				189.14		92.71657

				189.16		92.7108

				189.19		92.70503

				189.21		92.69926

				189.23		92.69348

				189.25		92.69348

				189.27		92.69348

				189.29		92.68771

				189.31		92.6704

				189.33		92.6704

				189.35		92.6704

				189.37		92.65886

				189.39		92.65886

				189.42		92.64731

				189.44		92.64731

				189.46		92.63

				189.48		92.63

				189.5		92.62423

				189.52		92.60691

				189.54		92.60114

				189.56		92.60691

				189.58		92.58383

				189.6		92.58383

				189.62		92.58383

				189.64		92.58383

				189.67		92.56651

				189.69		92.56651

				189.71		92.56651

				189.73		92.55497

				189.75		92.5492

				189.77		92.54343

				189.79		92.53766

				189.81		92.53189

				189.83		92.53189

				189.85		92.52034

				189.87		92.50303

				189.9		92.49726

				189.92		92.50303

				189.94		92.48572

				189.96		92.48572

				189.98		92.47994

				190		92.4684

				190.02		92.4684

				190.04		92.46263

				190.06		92.45109

				190.08		92.43955

				190.1		92.43955

				190.13		92.428

				190.15		92.41646

				190.17		92.41069

				190.19		92.39915

				190.21		92.39337

				190.23		92.39337

				190.25		92.3876

				190.27		92.37606

				190.29		92.37606

				190.31		92.37606

				190.33		92.37606

				190.36		92.37029

				190.38		92.36452

				190.4		92.36452

				190.42		92.36452

				190.44		92.35298

				190.46		92.34143

				190.48		92.33566

				190.5		92.33566

				190.52		92.31258

				190.54		92.31258

				190.56		92.30103

				190.59		92.28372

				190.61		92.27795

				190.63		92.26641

				190.65		92.26063

				190.67		92.25486

				190.69		92.25486

				190.71		92.24909

				190.73		92.23755

				190.75		92.23755

				190.77		92.22601

				190.79		92.22601

				190.82		92.23178

				190.84		92.23178

				190.86		92.22023

				190.88		92.21446

				190.9		92.21446

				190.92		92.20869

				190.94		92.19715

				190.96		92.19138

				190.98		92.18561

				191		92.16252

				191.02		92.15675

				191.05		92.17983

				191.07		92.15675

				191.09		92.18561

				191.11		92.16252

				191.13		92.16252

				191.15		92.15098

				191.17		92.14521

				191.19		92.12789

				191.21		92.13944

				191.23		92.15098

				191.25		92.13366

				191.28		92.09904

				191.3		92.10481

				191.32		92.05864

				191.34		92.08172

				191.36		92.06441

				191.38		92.07018

				191.4		92.05864

				191.42		92.05864

				191.44		92.02978

				191.46		92.03555

				191.48		92.03555

				191.51		92.02978

				191.53		92.01824

				191.55		92.01824

				191.57		92.00092

				191.59		92.00669

				191.61		91.97784

				191.63		91.98361

				191.65		91.97784

				191.67		91.97784

				191.69		91.9663

				191.71		91.96052

				191.74		91.95475

				191.76		91.94321

				191.78		91.93744

				191.8		91.93744

				191.82		91.9259

				191.84		91.93167

				191.86		91.91435

				191.88		91.91435

				191.9		91.90858

				191.92		91.90281

				191.94		91.89127

				191.96		91.89127

				191.99		91.89127

				192.01		91.87973

				192.03		91.87395

				192.05		91.86241

				192.07		91.85087

				192.09		91.85664

				192.11		91.83933

				192.13		91.83355

				192.15		91.82778

				192.17		91.82201

				192.19		91.81624

				192.22		91.81624

				192.24		91.81047

				192.26		91.8047

				192.28		91.79893

				192.3		91.79893

				192.32		91.78738

				192.34		91.77584

				192.36		91.78161

				192.38		91.75276

				192.4		91.75276

				192.42		91.74121

				192.44		91.7239

				192.47		91.71236

				192.49		91.71236

				192.51		91.70659

				192.53		91.69504

				192.55		91.6835

				192.57		91.68927

				192.59		91.67773

				192.61		91.67196

				192.63		91.6835

				192.65		91.66619

				192.67		91.65464

				192.7		91.65464

				192.72		91.6431

				192.74		91.62579

				192.76		91.62579

				192.78		91.62002

				192.8		91.62002

				192.82		91.6027

				192.84		91.60847

				192.86		91.60847

				192.88		91.58539

				192.9		91.59693

				192.92		91.58539

				192.95		91.5623

				192.97		91.55653

				192.99		91.54499

				193.01		91.53922

				193.03		91.5219

				193.05		91.49882

				193.07		91.51036

				193.09		91.48727

				193.11		91.48727

				193.13		91.50459

				193.15		91.48727

				193.18		91.4815

				193.2		91.4815

				193.22		91.4815

				193.24		91.4815

				193.26		91.46419

				193.28		91.46419

				193.3		91.45265

				193.32		91.42956

				193.34		91.42956

				193.36		91.41802

				193.38		91.40648

				193.4		91.4007

				193.43		91.39493

				193.45		91.38916

				193.47		91.37185

				193.49		91.36608

				193.51		91.36608

				193.53		91.37185

				193.55		91.36608

				193.57		91.35453

				193.59		91.3603

				193.61		91.34876

				193.63		91.34876

				193.66		91.33722

				193.68		91.33722

				193.7		91.33145

				193.72		91.31413

				193.74		91.30259

				193.76		91.29105

				193.78		91.27951

				193.8		91.25642

				193.82		91.25642

				193.84		91.25065

				193.86		91.24488

				193.88		91.23911

				193.91		91.24488

				193.93		91.23334

				193.95		91.22179

				193.97		91.23334

				193.99		91.23911

				194.01		91.22756

				194.03		91.22179

				194.05		91.22179

				194.07		91.20448

				194.09		91.19294

				194.11		91.18139

				194.14		91.19294

				194.16		91.16408

				194.18		91.15254

				194.2		91.15831

				194.22		91.12945

				194.24		91.12368

				194.26		91.14099

				194.28		91.13522

				194.3		91.11214

				194.32		91.12368

				194.34		91.11791

				194.36		91.10637

				194.39		91.09482

				194.41		91.11214

				194.43		91.08905

				194.45		91.07174

				194.47		91.0602

				194.49		91.07174

				194.51		91.03711

				194.53		91.03711

				194.55		91.03711

				194.57		91.01402

				194.59		91.00248

				194.62		90.99094

				194.64		90.98517

				194.66		90.9794

				194.68		90.9794

				194.7		90.97362

				194.72		90.95631

				194.74		90.95054

				194.76		90.95054

				194.78		90.94477

				194.8		90.94477

				194.82		90.94477

				194.85		90.92168

				194.87		90.91014

				194.89		90.91591

				194.91		90.91014

				194.93		90.8986

				194.95		90.89283

				194.97		90.88128

				194.99		90.87551

				195.01		90.8582

				195.03		90.8582

				195.05		90.85243

				195.07		90.84088

				195.1		90.83511

				195.12		90.82934

				195.14		90.8178

				195.16		90.80626

				195.18		90.80048

				195.2		90.78317

				195.22		90.78317

				195.24		90.77163

				195.26		90.76009

				195.28		90.737

				195.3		90.72546

				195.33		90.71969

				195.35		90.71969

				195.37		90.70237

				195.39		90.71969

				195.41		90.70237

				195.43		90.69083

				195.45		90.67929

				195.47		90.69083

				195.49		90.67352

				195.51		90.66197

				195.53		90.6562

				195.56		90.64466

				195.58		90.63312

				195.6		90.62734

				195.62		90.6158

				195.64		90.61003

				195.66		90.60426

				195.68		90.59849

				195.7		90.59849

				195.72		90.5754

				195.74		90.5754

				195.76		90.56386

				195.79		90.56386

				195.81		90.55232

				195.83		90.56386

				195.85		90.54655

				195.87		90.54077

				195.89		90.54077

				195.91		90.54077

				195.93		90.52346

				195.95		90.52923

				195.97		90.51192

				195.99		90.50615

				196.01		90.48306

				196.04		90.47729

				196.06		90.46575

				196.08		90.44266

				196.1		90.43689

				196.12		90.43112

				196.14		90.41381

				196.16		90.40226

				196.18		90.40226

				196.2		90.39072

				196.22		90.37918

				196.24		90.37918

				196.27		90.37341

				196.29		90.37341

				196.31		90.36763

				196.33		90.36763

				196.35		90.35032

				196.37		90.33878

				196.39		90.33878

				196.41		90.33878

				196.43		90.32146

				196.45		90.32146

				196.47		90.30415

				196.5		90.29261

				196.52		90.28106

				196.54		90.28106

				196.56		90.26952

				196.58		90.25798

				196.6		90.24644

				196.62		90.24066

				196.64		90.22335

				196.66		90.22912

				196.68		90.22335

				196.7		90.20604

				196.72		90.19449

				196.75		90.19449

				196.77		90.18872

				196.79		90.16564

				196.81		90.16564

				196.83		90.15987

				196.85		90.14832

				196.87		90.14255

				196.89		90.13678

				196.91		90.13101

				196.93		90.11947

				196.95		90.12524

				196.98		90.11947

				197		90.10792

				197.02		90.10215

				197.04		90.08484

				197.06		90.0733

				197.08		90.06175

				197.1		90.06175

				197.12		90.04444

				197.14		90.02713

				197.16		90.01558

				197.18		90.00981

				197.2		89.99827

				197.23		90.00981

				197.25		89.97518

				197.27		89.96364

				197.29		89.96941

				197.31		89.96364

				197.33		89.94633

				197.35		89.94633

				197.37		89.91747

				197.39		89.94633

				197.41		89.94056

				197.43		89.91747

				197.46		89.90593

				197.48		89.90593

				197.5		89.90016

				197.52		89.89438

				197.54		89.88284

				197.56		89.85976

				197.58		89.85976

				197.6		89.84244

				197.62		89.83667

				197.64		89.81936

				197.66		89.81359

				197.68		89.80204

				197.71		89.80204

				197.73		89.77896

				197.75		89.77896

				197.77		89.77896

				197.79		89.76742

				197.81		89.76742

				197.83		89.75587

				197.85		89.76164

				197.87		89.76164

				197.89		89.74433

				197.91		89.74433

				197.93		89.72124

				197.96		89.7097

				197.98		89.70393

				198		89.69239

				198.02		89.65776

				198.04		89.65776

				198.06		89.62313

				198.08		89.63467

				198.1		89.61159

				198.12		89.61159

				198.14		89.60582

				198.16		89.5885

				198.19		89.5885

				198.21		89.59427

				198.23		89.57696

				198.25		89.56542

				198.27		89.56542

				198.29		89.54233

				198.31		89.55388

				198.33		89.53656

				198.35		89.52502

				198.37		89.51348

				198.39		89.51925

				198.41		89.49616

				198.44		89.49616

				198.46		89.49616

				198.48		89.47885

				198.5		89.46153

				198.52		89.44422

				198.54		89.43845

				198.56		89.42113

				198.58		89.41536

				198.6		89.39228

				198.62		89.39805

				198.64		89.39228

				198.66		89.37496

				198.69		89.36342

				198.71		89.36342

				198.73		89.33456

				198.75		89.34611

				198.77		89.31725

				198.79		89.30571

				198.81		89.30571

				198.83		89.29994

				198.85		89.28839

				198.87		89.29417

				198.89		89.27108

				198.92		89.27685

				198.94		89.27108

				198.96		89.27108

				198.98		89.26531

				199		89.25377

				199.02		89.24222

				199.04		89.24222

				199.06		89.22491

				199.08		89.19605

				199.1		89.20182

				199.12		89.17874

				199.14		89.17874

				199.17		89.15565

				199.19		89.14988

				199.21		89.14411

				199.23		89.13257

				199.25		89.11525

				199.27		89.09217

				199.29		89.08063

				199.31		89.0864

				199.33		89.05754

				199.35		89.05177

				199.37		89.05177

				199.4		89.046

				199.42		89.04023

				199.44		89.04023

				199.46		89.02868

				199.48		89.02868

				199.5		89.02291

				199.52		89.0056

				199.54		88.99406

				199.56		88.99983

				199.58		88.9652

				199.6		88.94211

				199.62		88.93634

				199.65		88.91326

				199.67		88.91903

				199.69		88.91326

				199.71		88.89594

				199.73		88.89017

				199.75		88.89594

				199.77		88.89017

				199.79		88.87286

				199.81		88.87286

				199.83		88.86709

				199.85		88.87286

				199.87		88.86709

				199.9		88.86131

				199.92		88.84977

				199.94		88.86131

				199.96		88.82669

				199.98		88.82669

				200		88.78629

				200.02		88.78629

				200.04		88.78052

				200.06		88.77474

				200.08		88.74589

				200.1		88.74589

				200.13		88.72857

				200.15		88.71126

				200.17		88.69972

				200.19		88.68817

				200.21		88.67086

				200.23		88.65932

				200.25		88.65355

				200.27		88.642

				200.29		88.64778

				200.31		88.62469

				200.33		88.62469

				200.35		88.61892

				200.38		88.61315

				200.4		88.6016

				200.42		88.59006

				200.44		88.58429

				200.46		88.58429

				200.48		88.58429

				200.5		88.56121

				200.52		88.56121

				200.54		88.54389

				200.56		88.53812

				200.58		88.51503

				200.61		88.51503

				200.63		88.49772

				200.65		88.49772

				200.67		88.47463

				200.69		88.49195

				200.71		88.47463

				200.73		88.46309

				200.75		88.45155

				200.77		88.44001

				200.79		88.42269

				200.81		88.42269

				200.83		88.39961

				200.86		88.39961

				200.88		88.39961

				200.9		88.38229

				200.92		88.37652

				200.94		88.35921

				200.96		88.34767

				200.98		88.33035

				201		88.31881

				201.02		88.29572

				201.04		88.29572

				201.06		88.27841

				201.09		88.26687

				201.11		88.2611

				201.13		88.24955

				201.15		88.2207

				201.17		88.21492

				201.19		88.20338

				201.21		88.19761

				201.23		88.19184

				201.25		88.18607

				201.27		88.17453

				201.29		88.17453

				201.31		88.16875

				201.34		88.16298

				201.36		88.1399

				201.38		88.12258

				201.4		88.12835

				201.42		88.11681

				201.44		88.0995

				201.46		88.08796

				201.48		88.08218

				201.5		88.06487

				201.52		88.07064

				201.54		88.04756

				201.57		88.04178

				201.59		88.03601

				201.61		88.03024

				201.63		88.00716

				201.65		88.00716

				201.67		87.98984

				201.69		87.96099

				201.71		87.94367

				201.73		87.92636

				201.75		87.92636

				201.77		87.90327

				201.8		87.8975

				201.82		87.88596

				201.84		87.88596

				201.86		87.86864

				201.88		87.86287

				201.9		87.8571

				201.92		87.8571

				201.94		87.83979

				201.96		87.83402

				201.98		87.82247

				202		87.82247

				202.02		87.79939

				202.05		87.78785

				202.07		87.77053

				202.09		87.75899

				202.11		87.7359

				202.13		87.72436

				202.15		87.72436

				202.17		87.71282

				202.19		87.70705

				202.21		87.68973

				202.23		87.6955

				202.25		87.70128

				202.28		87.68396

				202.3		87.66665

				202.32		87.67242

				202.34		87.66665

				202.36		87.66088

				202.38		87.64356

				202.4		87.62625

				202.42		87.62625

				202.44		87.61471

				202.46		87.60316

				202.48		87.58008

				202.51		87.57431

				202.53		87.55699

				202.55		87.55122

				202.57		87.53391

				202.59		87.52236

				202.61		87.51082

				202.63		87.49928

				202.65		87.47042

				202.67		87.47619

				202.69		87.45311

				202.71		87.43579

				202.74		87.44157

				202.76		87.42425

				202.78		87.41271

				202.8		87.41271

				202.82		87.39539

				202.84		87.38962

				202.86		87.37808

				202.88		87.36077

				202.9		87.36077

				202.92		87.33768

				202.94		87.32037

				202.96		87.3146

				202.99		87.30305

				203.01		87.28574

				203.03		87.28574

				203.05		87.26843

				203.07		87.25688

				203.09		87.25688

				203.11		87.2338

				203.13		87.24534

				203.15		87.22225

				203.17		87.18185

				203.19		87.18763

				203.22		87.16454

				203.24		87.14146

				203.26		87.12414

				203.28		87.14723

				203.3		87.12991

				203.32		87.12414

				203.34		87.10683

				203.36		87.11837

				203.38		87.07797

				203.4		87.0722

				203.42		87.04911

				203.45		87.06066

				203.47		87.01449

				203.49		87.02026

				203.51		87.00294

				203.53		86.99717

				203.55		86.99717

				203.57		86.9914

				203.59		86.9914

				203.61		86.98563

				203.63		86.97986

				203.65		86.95677

				203.67		86.93946

				203.7		86.92214

				203.72		86.92214

				203.74		86.88752

				203.76		86.89906

				203.78		86.88752

				203.8		86.87597

				203.82		86.86443

				203.84		86.87597

				203.86		86.82403

				203.88		86.83557

				203.9		86.80672

				203.93		86.7894

				203.95		86.76632

				203.97		86.75478

				203.99		86.73169

				204.01		86.72592

				204.03		86.71438

				204.05		86.69706

				204.07		86.70283

				204.09		86.67398

				204.11		86.65666

				204.13		86.64512

				204.16		86.63935

				204.18		86.61049

				204.2		86.62781

				204.22		86.62203

				204.24		86.62203

				204.26		86.61049

				204.28		86.61626

				204.3		86.61626

				204.32		86.59318

				204.34		86.58164

				204.36		86.56432

				204.38		86.55278

				204.41		86.51238

				204.43		86.50661

				204.45		86.49507

				204.47		86.51238

				204.49		86.48352

				204.51		86.47198

				204.53		86.47198

				204.55		86.46044

				204.57		86.43158

				204.59		86.43158

				204.61		86.42581

				204.64		86.41427

				204.66		86.39118

				204.68		86.3681

				204.7		86.35078

				204.72		86.3681

				204.74		86.34501

				204.76		86.31615

				204.78		86.31038

				204.8		86.29884

				204.82		86.25844

				204.84		86.27575

				204.86		86.26998

				204.89		86.26998

				204.91		86.25844

				204.93		86.2469

				204.95		86.20073

				204.97		86.2065

				204.99		86.18341

				205.01		86.1661

				205.03		86.14301

				205.05		86.14301

				205.07		86.11993

				205.09		86.10839

				205.12		86.09107

				205.14		86.09684

				205.16		86.0853

				205.18		86.07376

				205.2		86.07953

				205.22		86.06222

				205.24		86.03913

				205.26		86.03336

				205.28		86.02182

				205.3		85.98719

				205.32		85.98719

				205.34		85.98142

				205.37		85.94679

				205.39		85.93525

				205.41		85.93525

				205.43		85.91216

				205.45		85.89485

				205.47		85.8833

				205.49		85.87753

				205.51		85.85445

				205.53		85.8429

				205.55		85.84868

				205.57		85.83713

				205.6		85.79673

				205.62		85.80828

				205.64		85.79096

				205.66		85.76211

				205.68		85.75056

				205.7		85.76211

				205.72		85.73902

				205.74		85.73325

				205.76		85.73325

				205.78		85.69862

				205.8		85.69285

				205.82		85.67554

				205.85		85.68131

				205.87		85.63514

				205.89		85.66976

				205.91		85.65245

				205.93		85.64668

				205.95		85.62359

				205.97		85.64668

				205.99		85.60628

				206.01		85.58897

				206.03		85.58897

				206.05		85.56011

				206.08		85.53702

				206.1		85.53125

				206.12		85.52548

				206.14		85.49085

				206.16		85.49085

				206.18		85.49085

				206.2		85.48508

				206.22		85.47931

				206.24		85.46777

				206.26		85.462

				206.28		85.41583

				206.3		85.39851

				206.33		85.3812

				206.35		85.36965

				206.37		85.35811

				206.39		85.34657

				206.41		85.32925

				206.43		85.31194

				206.45		85.29463

				206.47		85.28886

				206.49		85.28308

				206.51		85.28308

				206.53		85.27731

				206.56		85.26

				206.58		85.22537

				206.6		85.23114

				206.62		85.20806

				206.64		85.18497

				206.66		85.18497

				206.68		85.18497

				206.7		85.15611

				206.72		85.12726

				206.74		85.14457

				206.76		85.10994

				206.78		85.10994

				206.81		85.08109

				206.83		85.07532

				206.85		85.04646

				206.87		85.04069

				206.89		85.01183

				206.91		85.01183

				206.93		84.99452

				206.95		84.98297

				206.97		84.98875

				206.99		84.9772

				207.01		84.96566

				207.04		84.94835

				207.06		84.94258

				207.08		84.91372

				207.1		84.90218

				207.12		84.87909

				207.14		84.87332

				207.16		84.86178

				207.18		84.83869

				207.2		84.81561

				207.22		84.83292

				207.24		84.82715

				207.27		84.79252

				207.29		84.78675

				207.31		84.77521

				207.33		84.74635

				207.35		84.71172

				207.37		84.71749

				207.39		84.68864

				207.41		84.67709

				207.43		84.67132

				207.45		84.67709

				207.47		84.64247

				207.49		84.64247

				207.52		84.64247

				207.54		84.61938

				207.56		84.57898

				207.58		84.58475

				207.6		84.57321

				207.62		84.56167

				207.64		84.53858

				207.66		84.54435

				207.68		84.53281

				207.7		84.48087

				207.72		84.4751

				207.74		84.4751

				207.77		84.42893

				207.79		84.41738

				207.81		84.44047

				207.83		84.40007

				207.85		84.36544

				207.87		84.37698

				207.89		84.38853

				207.91		84.3539

				207.93		84.33081

				207.95		84.34813

				207.97		84.3135

				208		84.26733

				208.02		84.29619

				208.04		84.27887

				208.06		84.24424

				208.08		84.24424

				208.1		84.24424

				208.12		84.19807

				208.14		84.18076

				208.16		84.18653

				208.18		84.18076

				208.2		84.14036

				208.22		84.14036

				208.25		84.14036

				208.27		84.12304

				208.29		84.09996

				208.31		84.1115

				208.33		84.07687

				208.35		84.05956

				208.37		84.05956

				208.39		84.04802

				208.41		84.00762

				208.43		84.01916

				208.45		84.02493

				208.47		83.97299

				208.5		83.97299

				208.52		83.97299

				208.54		83.92682

				208.56		83.90373

				208.58		83.90373

				208.6		83.85756

				208.62		83.84025

				208.64		83.85179

				208.66		83.84025

				208.68		83.83448

				208.7		83.83448

				208.73		83.83448

				208.75		83.80562

				208.77		83.76522

				208.79		83.76522

				208.81		83.76522

				208.83		83.73059

				208.85		83.72482

				208.87		83.73637

				208.89		83.69019

				208.91		83.67288

				208.93		83.65557

				208.95		83.63248

				208.98		83.59785

				209		83.59785

				209.02		83.57477

				209.04		83.53437

				209.06		83.51705

				209.08		83.51705

				209.1		83.49974

				209.12		83.47665

				209.14		83.49397

				209.16		83.49397

				209.18		83.44203

				209.21		83.43048

				209.23		83.4478

				209.25		83.41317

				209.27		83.39586

				209.29		83.40163

				209.31		83.4074

				209.33		83.37277

				209.35		83.367

				209.37		83.35546

				209.39		83.34391

				209.41		83.30929

				209.43		83.30351

				209.46		83.29774

				209.48		83.25157

				209.5		83.25734

				209.52		83.24003

				209.54		83.2054

				209.56		83.19386

				209.58		83.19963

				209.6		83.14769

				209.62		83.1246

				209.64		83.11883

				209.66		83.10152

				209.69		83.0842

				209.71		83.07266

				209.73		83.0842

				209.75		83.06112

				209.77		83.0438

				209.79		83.04958

				209.81		83.04958

				209.83		83.01495

				209.85		83.01495

				209.87		83.00918

				209.89		82.98032

				209.92		82.94569

				209.94		82.97455

				209.96		82.93415

				209.98		82.91683

				210		82.90529

				210.02		82.89952

				210.04		82.83604

				210.06		82.83604

				210.08		82.81872

				210.1		82.80718

				210.12		82.76678

				210.14		82.77832

				210.17		82.76678

				210.19		82.73792

				210.21		82.72061

				210.23		82.76101

				210.25		82.71484

				210.27		82.69175

				210.29		82.68021

				210.31		82.66867

				210.33		82.61095

				210.35		82.59941

				210.37		82.61673

				210.4		82.5821

				210.42		82.55324

				210.44		82.54747

				210.46		82.54747

				210.48		82.46667

				210.5		82.48398

				210.52		82.44936

				210.54		82.4205

				210.56		82.40319

				210.58		82.43781

				210.6		82.39741

				210.63		82.40319

				210.65		82.39741

				210.67		82.3801

				210.69		82.33393

				210.71		82.3397

				210.73		82.33393

				210.75		82.2993

				210.77		82.2993

				210.79		82.2993

				210.81		82.28199

				210.83		82.23582

				210.85		82.25313

				210.88		82.22427

				210.9		82.18965

				210.92		82.16656

				210.94		82.16079

				210.96		82.11462

				210.98		82.10308

				211		82.10885

				211.02		82.07999

				211.04		82.05691

				211.06		82.06845

				211.08		82.05691

				211.11		82.01073

				211.13		82.01073

				211.15		81.99919

				211.17		81.95879

				211.19		81.91839

				211.21		81.97034

				211.23		81.92416

				211.25		81.90685

				211.27		81.90108

				211.29		81.92994

				211.31		81.83759

				211.33		81.84337

				211.36		81.84914

				211.38		81.83759

				211.4		81.77411

				211.42		81.7972

				211.44		81.77988

				211.46		81.73948

				211.48		81.68754

				211.5		81.69331

				211.52		81.67023

				211.54		81.62983

				211.56		81.64137

				211.59		81.65868

				211.61		81.61828

				211.63		81.60097

				211.65		81.61828

				211.67		81.56634

				211.69		81.53171

				211.71		81.53748

				211.73		81.53171

				211.75		81.49709

				211.77		81.46823

				211.79		81.49709

				211.81		81.46246

				211.84		81.44514

				211.86		81.44514

				211.88		81.44514

				211.9		81.37589

				211.92		81.37589

				211.94		81.37012

				211.96		81.34126

				211.98		81.31817

				212		81.32972

				212.02		81.30086

				212.04		81.25469

				212.07		81.26046

				212.09		81.26046

				212.11		81.23738

				212.13		81.20275

				212.15		81.22583

				212.17		81.1912

				212.19		81.15658

				212.21		81.17389

				212.23		81.16812

				212.25		81.12772

				212.27		81.1912

				212.3		81.22583

				212.32		81.17966

				212.34		81.16235

				212.36		81.13926

				212.38		81.02961

				212.4		80.93727

				212.42		80.90264

				212.44		80.89109

				212.46		80.87378

				212.48		80.87378

				212.5		80.93149

				212.53		80.91418

				212.55		80.90841

				212.57		80.93149

				212.59		80.87955

				212.61		80.78721

				212.63		80.7699

				212.65		80.7295

				212.67		80.65447

				212.69		80.61984

				212.71		80.66601

				212.73		80.63716

				212.75		80.63138

				212.78		80.63138

				212.8		80.66601

				212.82		80.60253

				212.84		80.57367

				212.86		80.68333

				212.88		80.71218

				212.9		80.58521

				212.92		80.61407

				212.94		80.66024

				212.96		80.49864

				212.98		80.4467

				213.01		80.53904

				213.03		80.50442

				213.05		80.45824

				213.07		80.48133

				213.09		80.45824

				213.11		80.45824

				213.13		80.43516

				213.15		80.4467

				213.17		80.40053

				213.19		80.37167

				213.21		80.34859

				213.24		80.3255

				213.26		80.27933

				213.28		80.26779

				213.3		80.26202

				213.32		80.22739

				213.34		80.20431

				213.36		80.19853

				213.38		80.16968

				213.4		80.15813

				213.42		80.15236

				213.44		80.12928

				213.46		80.12351

				213.49		80.10042

				213.51		80.08311

				213.53		80.04271

				213.55		80.03694

				213.57		80.00231

				213.59		79.98499

				213.61		79.96191

				213.63		79.95614

				213.65		79.9446

				213.67		79.92151

				213.69		79.90997

				213.72		79.89265

				213.74		79.87534

				213.76		79.84648

				213.78		79.84071

				213.8		79.81763

				213.82		79.79454

				213.84		79.76568

				213.86		79.76568

				213.88		79.7426

				213.9		79.72528

				213.92		79.70797

				213.95		79.68488

				213.97		79.65026

				213.99		79.65026

				214.01		79.64449

				214.03		79.60409

				214.05		79.58677

				214.07		79.58677

				214.09		79.54637

				214.11		79.52329

				214.13		79.52329

				214.15		79.52906

				214.17		79.50597

				214.2		79.48289

				214.22		79.46557

				214.24		79.47712

				214.26		79.44826

				214.28		79.4194

				214.3		79.44249

				214.32		79.41363

				214.34		79.36746

				214.36		79.35592

				214.38		79.3386

				214.4		79.28089

				214.43		79.28089

				214.45		79.25781

				214.47		79.20586

				214.49		79.18855

				214.51		79.17124

				214.53		79.12506

				214.55		79.11929

				214.57		79.11352

				214.59		79.09621

				214.61		79.06735

				214.63		79.07312

				214.66		79.05581

				214.68		79.02695

				214.7		79.02118

				214.72		79.00387

				214.74		78.98655

				214.76		78.95192

				214.78		78.93461

				214.8		78.92307

				214.82		78.88844

				214.84		78.88267

				214.86		78.88267

				214.89		78.86535

				214.91		78.84227

				214.93		78.84227

				214.95		78.79033

				214.97		78.7557

				214.99		78.76724

				215.01		78.74416

				215.03		78.69799

				215.05		78.69799

				215.07		78.68644

				215.09		78.64027

				215.12		78.61719

				215.14		78.62296

				215.16		78.59987

				215.18		78.57679

				215.2		78.58256

				215.22		78.54216

				215.24		78.53639

				215.26		78.5133

				215.28		78.49599

				215.3		78.46713

				215.32		78.43828

				215.35		78.40942

				215.37		78.38633

				215.39		78.36325

				215.41		78.32862

				215.43		78.34016

				215.45		78.31131

				215.47		78.28822

				215.49		78.28245

				215.51		78.25359

				215.53		78.21896

				215.55		78.20742

				215.58		78.21319

				215.6		78.17857

				215.62		78.13817

				215.64		78.14971

				215.66		78.11508

				215.68		78.092

				215.7		78.06314

				215.72		78.092

				215.74		78.04005

				215.76		78.04005

				215.78		78.01697

				215.81		78.0112

				215.83		77.9708

				215.85		77.95925

				215.87		77.91885

				215.89		77.90154

				215.91		77.87268

				215.93		77.86114

				215.95		77.82651

				215.97		77.81497

				215.99		77.79766

				216.01		77.78034

				216.03		77.7688

				216.06		77.75149

				216.08		77.72263

				216.1		77.69377

				216.12		77.67646

				216.14		77.65337

				216.16		77.63029

				216.18		77.61297

				216.2		77.61297

				216.22		77.58989

				216.24		77.5668

				216.26		77.56103

				216.29		77.5264

				216.31		77.49178

				216.33		77.50332

				216.35		77.46869

				216.37		77.42829

				216.39		77.41098

				216.41		77.39943

				216.43		77.35904

				216.45		77.33595

				216.47		77.33018

				216.49		77.32441

				216.51		77.28978

				216.54		77.24938

				216.56		77.24361

				216.58		77.22629

				216.6		77.19744

				216.62		77.16281

				216.64		77.18012

				216.66		77.12818

				216.68		77.11087

				216.7		77.09355

				216.72		77.09932

				216.74		77.04738

				216.77		77.05315

				216.79		77.03007

				216.81		77.01853

				216.83		76.97236

				216.85		76.97236

				216.87		76.96658

				216.89		76.93196

				216.91		76.90887

				216.93		76.9031

				216.95		76.88001

				216.97		76.83384

				216.99		76.84539

				217.02		76.80499

				217.04		76.7819

				217.06		76.7415

				217.08		76.7415

				217.1		76.7011

				217.12		76.67802

				217.14		76.63762

				217.16		76.64916

				217.18		76.60299

				217.2		76.59722

				217.22		76.59145

				217.25		76.5799

				217.27		76.55105

				217.29		76.5395

				217.31		76.49911

				217.33		76.47025

				217.35		76.44139

				217.37		76.40676

				217.39		76.38945

				217.41		76.37214

				217.43		76.35482

				217.45		76.32597

				217.48		76.32597

				217.5		76.28557

				217.52		76.27402

				217.54		76.26248

				217.56		76.22785

				217.58		76.20477

				217.6		76.18745

				217.62		76.17014

				217.64		76.12974

				217.66		76.12974

				217.68		76.09511

				217.71		76.08934

				217.73		76.04317

				217.75		76.06048

				217.77		76.02008

				217.79		75.997

				217.81		75.9566

				217.83		75.95083

				217.85		75.89311

				217.87		75.88734

				217.89		75.86426

				217.91		75.84694

				217.94		75.82386

				217.96		75.81809

				217.98		75.795

				218		75.77192

				218.02		75.74883

				218.04		75.7546

				218.06		75.70266

				218.08		75.69112

				218.1		75.66226

				218.12		75.65072

				218.14		75.59878

				218.16		75.59878

				218.19		75.57569

				218.21		75.54106

				218.23		75.52952

				218.25		75.51798

				218.27		75.50066

				218.29		75.46604

				218.31		75.47758

				218.33		75.44872

				218.35		75.41986

				218.37		75.41409

				218.39		75.39678

				218.42		75.35638

				218.44		75.34484

				218.46		75.32752

				218.48		75.27558

				218.5		75.2525

				218.52		75.22364

				218.54		75.21787

				218.56		75.16015

				218.58		75.16015

				218.6		75.1313

				218.62		75.11976

				218.65		75.06781

				218.67		75.08513

				218.69		75.04473

				218.71		75.03896

				218.73		75.00433

				218.75		74.98701

				218.77		74.94662

				218.79		74.94662

				218.81		74.90622

				218.83		74.88313

				218.85		74.86005

				218.87		74.8485

				218.9		74.80233

				218.92		74.79079

				218.94		74.77347

				218.96		74.73885

				218.98		74.72153

				219		74.72153

				219.02		74.73308

				219.04		74.64651

				219.06		74.65805

				219.08		74.60611

				219.1		74.55994

				219.13		74.47337

				219.15		74.51954

				219.17		74.45605

				219.19		74.46182

				219.21		74.45605

				219.23		74.48491

				219.25		74.43874

				219.27		74.43874

				219.29		74.39834

				219.31		74.3868

				219.33		74.31754

				219.35		74.31177

				219.38		74.30023

				219.4		74.27137

				219.42		74.24251

				219.44		74.24251

				219.46		74.21365

				219.48		74.17903

				219.5		74.1444

				219.52		74.12708

				219.54		74.104

				219.56		74.07514

				219.58		74.03474

				219.61		74.05206

				219.63		74.05206

				219.65		74.01166

				219.67		74.00589

				219.69		73.98857

				219.71		73.90777

				219.73		73.85006

				219.75		73.8212

				219.77		73.77503

				219.79		73.74041

				219.81		73.72309

				219.83		73.70001

				219.86		73.66538

				219.88		73.65961

				219.9		73.64229

				219.92		73.63652

				219.94		73.61921

				219.96		73.60189

				219.98		73.60189

				220		73.57881

				220.02		73.56726

				220.04		73.53264

				220.06		73.53264

				220.09		73.49224

				220.11		73.48647

				220.13		73.45184

				220.15		73.44607

				220.17		73.3999

				220.19		73.36527

				220.21		73.34795

				220.23		73.30755

				220.25		73.26138

				220.27		73.18636

				220.29		73.2383

				220.31		73.30178

				220.34		73.22098

				220.36		73.22676

				220.38		73.24407

				220.4		73.14596

				220.42		73.02476

				220.44		73.08824

				220.46		73.04207

				220.48		73.03053

				220.5		73.04784

				220.52		73.01322

				220.54		72.96127

				220.57		72.94396

				220.59		72.93242

				220.61		72.8747

				220.63		72.86316

				220.65		72.86893

				220.67		72.8747

				220.69		72.82853

				220.71		72.78813

				220.73		72.75351

				220.75		72.70734

				220.77		72.63808

				220.8		72.60345

				220.82		72.60345

				220.84		72.56305

				220.86		72.55151

				220.88		72.53997

				220.9		72.52265

				220.92		72.48802

				220.94		72.47071

				220.96		72.4534

				220.98		72.413

				221		72.39568

				221.03		72.36683

				221.05		72.33797

				221.07		72.27448

				221.09		72.211

				221.11		72.28603

				221.13		72.14752

				221.15		72.1706

				221.17		72.16483

				221.19		72.18791

				221.21		72.06095

				221.23		72.15329

				221.26		72.08403

				221.28		72.06672

				221.3		72.03786

				221.32		72.03786

				221.34		72.009

				221.36		71.97438

				221.38		71.95129

				221.4		71.91089

				221.42		71.87626

				221.44		71.85895

				221.46		71.83586

				221.49		71.81855

				221.51		71.78969

				221.53		71.77815

				221.55		71.72044

				221.57		71.72044

				221.59		71.68004

				221.61		71.67427

				221.63		71.63387

				221.65		71.66272

				221.67		71.59924

				221.69		71.5877

				221.72		71.55884

				221.74		71.51267

				221.76		71.48958

				221.78		71.46073

				221.8		71.43764

				221.82		71.42033

				221.84		71.40301

				221.86		71.3453

				221.88		71.33953

				221.9		71.3049

				221.92		71.27027

				221.95		71.25296

				221.97		71.22987

				221.99		71.1837

				222.01		71.17216

				222.03		71.14907

				222.05		71.12022

				222.07		71.09136

				222.09		71.08559

				222.11		71.04519

				222.13		70.99902

				222.15		70.99325

				222.18		70.95285

				222.2		70.91822

				222.22		70.89513

				222.24		70.89513

				222.26		70.83165

				222.28		70.82011

				222.3		70.77394

				222.32		70.75085

				222.34		70.71045

				222.36		70.71045

				222.38		70.67582

				222.41		70.66428

				222.43		70.61811

				222.45		70.58925

				222.47		70.57194

				222.49		70.54308

				222.51		70.52

				222.53		70.51423

				222.55		70.49114

				222.57		70.4392

				222.59		70.43343

				222.62		70.40457

				222.64		70.36994

				222.66		70.3584

				222.68		70.34109

				222.7		70.29492

				222.72		70.27183

				222.74		70.26029

				222.76		70.21989

				222.78		70.18526

				222.8		70.15063

				222.82		70.13332

				222.85		70.08715

				222.87		70.06406

				222.89		70.02366

				222.91		70.02366

				222.93		69.97749

				222.95		69.96595

				222.97		69.90824

				222.99		69.89669

				223.01		69.87361

				223.03		69.85629

				223.05		69.81012

				223.08		69.81589

				223.1		69.78127

				223.12		69.74087

				223.14		69.6947

				223.16		69.70624

				223.18		69.6543

				223.2		69.63698

				223.22		69.6139

				223.24		69.61967

				223.26		69.54464

				223.28		69.5331

				223.31		69.51578

				223.33		69.47539

				223.35		69.43499

				223.37		69.44076

				223.39		69.39459

				223.41		69.34842

				223.43		69.32533

				223.45		69.29647

				223.47		69.24453

				223.49		69.24453

				223.52		69.22145

				223.54		69.19259

				223.56		69.15219

				223.58		69.15219

				223.6		69.12333

				223.62		69.09448

				223.64		69.05985

				223.66		69.07139

				223.68		69.01368

				223.7		68.97328

				223.72		68.96174

				223.75		68.93288

				223.77		68.86939

				223.79		68.86362

				223.81		68.81745

				223.83		68.78282

				223.85		68.75397

				223.87		68.7482

				223.89		68.69625

				223.91		68.67894

				223.93		68.65586

				223.96		68.63277

				223.98		68.59237

				224		68.60391

				224.02		68.58083

				224.04		68.5462

				224.06		68.5058

				224.08		68.48849

				224.1		68.45386

				224.12		68.41346

				224.14		68.39614

				224.17		68.3846

				224.19		68.3442

				224.21		68.3038

				224.23		68.29226

				224.25		68.24609

				224.27		68.21146

				224.29		68.18261

				224.31		68.15952

				224.33		68.10758

				224.35		68.07295

				224.37		68.05564

				224.4		68.00946

				224.42		67.96329

				224.44		67.95752

				224.46		67.93444

				224.48		67.88827

				224.5		67.87672

				224.52		67.85941

				224.54		67.81324

				224.56		67.78438

				224.58		67.7613

				224.61		67.74975

				224.63		67.71513

				224.65		67.69204

				224.67		67.68627

				224.69		67.6401

				224.71		67.5997

				224.73		67.58239

				224.75		67.55353

				224.77		67.49582

				224.79		67.50159

				224.82		67.45542

				224.84		67.42079

				224.86		67.37462

				224.88		67.35153

				224.9		67.29959

				224.92		67.27073

				224.94		67.24188

				224.96		67.22456

				224.98		67.17262

				225		67.16108

				225.02		67.16685

				225.05		67.11491

				225.07		67.09759

				225.09		67.09182

				225.11		67.08028

				225.13		67.02257

				225.15		66.99948

				225.17		66.97062

				225.19		66.936

				225.21		66.88983

				225.23		66.88405

				225.26		66.86097

				225.28		66.80903

				225.3		66.79748

				225.32		66.75131

				225.34		66.71091

				225.36		66.67629

				225.38		66.67051

				225.4		66.58972

				225.42		66.56086

				225.44		66.54354

				225.47		66.50315

				225.49		66.46275

				225.51		66.47429

				225.53		66.46852

				225.55		66.41658

				225.57		66.39349

				225.59		66.37618

				225.61		66.34155

				225.63		66.28961

				225.65		66.27229

				225.67		66.26652

				225.7		66.20304

				225.72		66.17418

				225.74		66.16264

				225.76		66.09915

				225.78		66.05298

				225.8		66.04144

				225.82		66.01835

				225.84		65.96064

				225.86		65.96064

				225.88		65.93178

				225.91		65.91447

				225.93		65.85676

				225.95		65.85098

				225.97		65.81058

				225.99		65.79327

				226.01		65.74133

				226.03		65.74133

				226.05		65.68362

				226.07		65.67784

				226.09		65.64899

				226.12		65.63167

				226.14		65.57973

				226.16		65.57396

				226.18		65.51625

				226.2		65.47008

				226.22		65.45276

				226.24		65.40659

				226.26		65.36042

				226.28		65.33733

				226.3		65.32002

				226.32		65.26808

				226.35		65.23922

				226.37		65.21614

				226.39		65.19305

				226.41		65.13534

				226.43		65.13534

				226.45		65.11802

				226.47		65.07762

				226.49		65.05454

				226.51		65.05454

				226.53		64.99683

				226.56		64.9622

				226.58		64.95643

				226.6		64.91026

				226.62		64.87563

				226.64		64.83523

				226.66		64.81791

				226.68		64.74289

				226.7		64.69672

				226.72		64.66209

				226.74		64.639

				226.77		64.59283

				226.79		64.57552

				226.81		64.57552

				226.83		64.5178

				226.85		64.46586

				226.87		64.45432

				226.89		64.42546

				226.91		64.35621

				226.93		64.35621

				226.95		64.35044

				226.97		64.30427

				227		64.24655

				227.02		64.26387

				227.04		64.21769

				227.06		64.17152

				227.08		64.14844

				227.1		64.14267

				227.12		64.08495

				227.14		64.04455

				227.16		64.02147

				227.18		63.98107

				227.21		63.92336

				227.23		63.90027

				227.25		63.85987

				227.27		63.82524

				227.29		63.78484

				227.31		63.7733

				227.33		63.72136

				227.35		63.67519

				227.37		63.65787

				227.39		63.62902

				227.41		63.60016

				227.44		63.57708

				227.46		63.5713

				227.48		63.52513

				227.5		63.49628

				227.52		63.45588

				227.54		63.44434

				227.56		63.38662

				227.58		63.37508

				227.6		63.32891

				227.62		63.28851

				227.65		63.24234

				227.67		63.21925

				227.69		63.15

				227.71		63.13268

				227.73		63.1096

				227.75		63.07497

				227.77		63.02303

				227.79		63.0288

				227.81		62.9884

				227.83		62.94223

				227.85		62.9076

				227.88		62.90183

				227.9		62.84412

				227.92		62.80372

				227.94		62.79795

				227.96		62.76909

				227.98		62.71138

				228		62.69406

				228.02		62.67098

				228.04		62.63058

				228.06		62.59595

				228.09		62.57863

				228.11		62.53246

				228.13		62.49206

				228.15		62.45167

				228.17		62.42281

				228.19		62.36509

				228.21		62.33047

				228.23		62.30161

				228.25		62.27275

				228.27		62.2035

				228.29		62.21504

				228.32		62.16887

				228.34		62.1227

				228.36		62.0823

				228.38		62.09961

				228.4		62.03036

				228.42		62.01881

				228.44		62.0015

				228.46		62.01881

				228.48		61.9611

				228.5		61.92647

				228.53		61.90339

				228.55		61.85722

				228.57		61.78219

				228.59		61.7591

				228.61		61.72448

				228.63		61.66676

				228.65		61.63791

				228.67		61.60905

				228.69		61.53979

				228.71		61.52248

				228.73		61.49362

				228.76		61.44745

				228.78		61.40705

				228.8		61.38974

				228.82		61.34934

				228.84		61.2974

				228.86		61.28008

				228.88		61.23968

				228.9		61.20506

				228.92		61.18774

				228.94		61.15311

				228.97		61.12426

				228.99		61.07809

				229.01		61.055

				229.03		60.99729

				229.05		60.97997

				229.07		60.92226

				229.09		60.91649

				229.11		60.84723

				229.13		60.8126

				229.15		60.78375

				229.17		60.74912

				229.2		60.67986

				229.22		60.68564

				229.24		60.63946

				229.26		60.61061

				229.28		60.55867

				229.3		60.55289

				229.32		60.51249

				229.34		60.4721

				229.36		60.42015

				229.38		60.42015

				229.41		60.36244

				229.43		60.33935

				229.45		60.3105

				229.47		60.28164

				229.49		60.22393

				229.51		60.20084

				229.53		60.14313

				229.55		60.10273

				229.57		60.06233

				229.59		60.02193

				229.62		59.96999

				229.64		59.92382

				229.66		59.88919

				229.68		59.83725

				229.7		59.82571

				229.72		59.77376

				229.74		59.76222

				229.76		59.73336

				229.78		59.70451

				229.8		59.65834

				229.82		59.64102

				229.85		59.61217

				229.87		59.58331

				229.89		59.56022

				229.91		59.53137

				229.93		59.50828

				229.95		59.46211

				229.97		59.43325

				229.99		59.37554

				230.01		59.35246

				230.03		59.28897

				230.05		59.24857

				230.08		59.19663

				230.1		59.19086

				230.12		59.12737

				230.14		59.10429

				230.16		59.08697

				230.18		59.03503

				230.2		58.97732

				230.22		58.97155

				230.24		58.93115

				230.26		58.90229

				230.29		58.87921

				230.31		58.86189

				230.33		58.82149

				230.35		58.78109

				230.37		58.75224

				230.39		58.70607

				230.41		58.65412

				230.43		58.60795

				230.45		58.59641

				230.47		58.54447

				230.49		58.51561

				230.52		58.49253

				230.54		58.46944

				230.56		58.39441

				230.58		58.36556

				230.6		58.33093

				230.62		58.27899

				230.64		58.22704

				230.66		58.20973

				230.68		58.15202

				230.7		58.10585

				230.73		58.06545

				230.75		58.01928

				230.77		57.96156

				230.79		57.90962

				230.81		57.87499

				230.83		57.81728

				230.85		57.77688

				230.87		57.75379

				230.89		57.73648

				230.91		57.70185

				230.93		57.70762

				230.96		57.68454

				230.98		57.64414

				231		57.62105

				231.02		57.56911

				231.04		57.52871

				231.06		57.47677

				231.08		57.45369

				231.1		57.41329

				231.12		57.38443

				231.14		57.34403

				231.17		57.32094

				231.19		57.26323

				231.21		57.22283

				231.23		57.19975

				231.25		57.15358

				231.27		57.10163

				231.29		57.08432

				231.31		57.03815

				231.33		56.98621

				231.35		56.94004

				231.37		56.92272

				231.4		56.85924

				231.42		56.83038

				231.44		56.79575

				231.46		56.75535

				231.48		56.70918

				231.5		56.69187

				231.52		56.65724

				231.54		56.61684

				231.56		56.59376

				231.58		56.55336

				231.61		56.49564

				231.63		56.46101

				231.65		56.42639

				231.67		56.38022

				231.69		56.34559

				231.71		56.33405

				231.73		56.29365

				231.75		56.25325

				231.77		56.20708

				231.79		56.17822

				231.81		56.11473

				231.84		56.08588

				231.86		56.03394

				231.88		56.02239

				231.9		55.97045

				231.92		55.94159

				231.94		55.88965

				231.96		55.87234

				231.98		55.80885

				232		55.76845

				232.02		55.7396

				232.05		55.70497

				232.07		55.64726

				232.09		55.62994

				232.11		55.578

				232.13		55.5376

				232.15		55.49143

				232.17		55.44526

				232.19		55.42217

				232.21		55.376

				232.23		55.3356

				232.25		55.2952

				232.28		55.28366

				232.3		55.20286

				232.32		55.19709

				232.34		55.15092

				232.36		55.10475

				232.38		55.05858

				232.4		55.03549

				232.42		54.98932

				232.44		54.94892

				232.46		54.90852

				232.49		54.87967

				232.51		54.82773

				232.53		54.78155

				232.55		54.74116

				232.57		54.72384

				232.59		54.65459

				232.61		54.62573

				232.63		54.5911

				232.65		54.54493

				232.67		54.50453

				232.7		54.46413

				232.72		54.41796

				232.74		54.37179

				232.76		54.34293

				232.78		54.29099

				232.8		54.25636

				232.82		54.21596

				232.84		54.18711

				232.86		54.13516

				232.89		54.10054

				232.91		54.07168

				232.93		54.02551

				232.95		53.97357

				232.97		53.93317

				232.99		53.90431

				233.01		53.85237

				233.03		53.81774

				233.05		53.78888

				233.07		53.7658

				233.1		53.69654

				233.12		53.67923

				233.14		53.63306

				233.16		53.58689

				233.18		53.54072

				233.2		53.52917

				233.22		53.47146

				233.24		53.41952

				233.26		53.37912

				233.28		53.34449

				233.31		53.28101

				233.33		53.24061

				233.35		53.21175

				233.37		53.16558

				233.39		53.10787

				233.41		53.08478

				233.43		53.04438

				233.45		52.99244

				233.47		52.94627

				233.49		52.93473

				233.52		52.87701

				233.54		52.84816

				233.56		52.80199

				233.58		52.78467

				233.6		52.72119

				233.62		52.69233

				233.64		52.62885

				233.66		52.60576

				233.68		52.54805

				233.7		52.50188

				233.73		52.4557

				233.75		52.40953

				233.77		52.37491

				233.79		52.31719

				233.81		52.29411

				233.83		52.23639

				233.85		52.20754

				233.87		52.17291

				233.89		52.14982

				233.91		52.09788

				233.94		52.06903

				233.96		52.02863

				233.98		51.97091

				234		51.92474

				234.02		51.87857

				234.04		51.83817

				234.06		51.80931

				234.08		51.76314

				234.1		51.72274

				234.12		51.68235

				234.15		51.64772

				234.17		51.59

				234.19		51.55538

				234.21		51.49766

				234.23		51.45726

				234.25		51.41686

				234.27		51.38224

				234.29		51.33029

				234.31		51.29567

				234.34		51.23795

				234.36		51.19755

				234.38		51.13984

				234.4		51.09944

				234.42		51.09367

				234.44		51.06481

				234.46		50.99556

				234.48		50.97247

				234.5		50.93784

				234.52		50.86282

				234.55		50.81087

				234.57		50.78779

				234.59		50.71853

				234.61		50.67236

				234.63		50.63196

				234.65		50.62619

				234.67		50.55116

				234.69		50.52808

				234.71		50.47614

				234.73		50.42996

				234.76		50.33762

				234.78		50.33185

				234.8		50.27991

				234.82		50.24528

				234.84		50.2222

				234.86		50.19911

				234.88		50.12408

				234.9		50.101

				234.92		50.0606

				234.94		49.99711

				234.97		49.9394

				234.99		49.899

				235.01		49.8586

				235.03		49.80089

				235.05		49.76626

				235.07		49.74318

				235.09		49.71432

				235.11		49.65083

				235.13		49.61043

				235.15		49.57004

				235.18		49.51809

				235.2		49.47192

				235.22		49.43152

				235.24		49.37381

				235.26		49.32764

				235.28		49.30455

				235.3		49.22375

				235.32		49.20067

				235.34		49.17181

				235.36		49.11987

				235.38		49.03907

				235.41		49.05061

				235.43		48.98136

				235.45		48.93519

				235.47		48.88325

				235.49		48.87747

				235.51		48.81399

				235.53		48.76205

				235.55		48.73896

				235.57		48.68125

				235.59		48.63508

				235.62		48.59468

				235.64		48.56582

				235.66		48.47925

				235.68		48.46194

				235.7		48.39845

				235.72		48.34651

				235.74		48.2888

				235.76		48.27726

				235.78		48.23108

				235.8		48.18491

				235.83		48.12143

				235.85		48.10989

				235.87		48.0464

				235.89		47.99446

				235.91		47.95406

				235.93		47.95406

				235.95		47.87903

				235.97		47.8444

				235.99		47.79823

				236.01		47.76938

				236.04		47.68281

				236.06		47.65395

				236.08		47.61932

				236.1		47.57892

				236.12		47.53852

				236.14		47.5039

				236.16		47.45772

				236.18		47.39424

				236.2		47.34807

				236.22		47.29036

				236.25		47.23841

				236.27		47.20379

				236.29		47.16916

				236.31		47.10567

				236.33		47.0595

				236.35		47.00756

				236.37		46.95562

				236.39		46.91522

				236.41		46.88636

				236.43		46.86328

				236.46		46.82288

				236.48		46.78248

				236.5		46.72476

				236.52		46.68437

				236.54		46.60357

				236.56		46.56894

				236.58		46.52854

				236.6		46.47083

				236.62		46.43043

				236.64		46.39003

				236.67		46.34386

				236.69		46.28037

				236.71		46.25151

				236.73		46.1938

				236.75		46.14763

				236.77		46.113

				236.79		46.0726

				236.81		46.01489

				236.83		45.97449

				236.85		45.92832

				236.88		45.87638

				236.9		45.81289

				236.92		45.77827

				236.94		45.75518

				236.96		45.69747

				236.98		45.66284

				237		45.63975

				237.02		45.57627

				237.04		45.50701

				237.06		45.46084

				237.09		45.41467

				237.11		45.35119

				237.13		45.31079

				237.15		45.2877

				237.17		45.23576

				237.19		45.17805

				237.21		45.13765

				237.23		45.09725

				237.25		45.02222

				237.27		44.99336

				237.3		44.94142

				237.32		44.88948

				237.34		44.82599

				237.36		44.82022

				237.38		44.75097

				237.4		44.68748

				237.42		44.65285

				237.44		44.61245

				237.46		44.53166

				237.48		44.5028

				237.51		44.47394

				237.53		44.422

				237.55		44.35852

				237.57		44.33543

				237.59		44.26617

				237.61		44.22

				237.63		44.16806

				237.65		44.10458

				237.67		44.04109

				237.69		44.00646

				237.72		43.96029

				237.74		43.90835

				237.76		43.87372

				237.78		43.85064

				237.8		43.80447

				237.82		43.72367

				237.84		43.68904

				237.86		43.66018

				237.88		43.57938

				237.9		43.52167

				237.93		43.5159

				237.95		43.44664

				237.97		43.38316

				237.99		43.3543

				238.01		43.30813

				238.03		43.22733

				238.05		43.18116

				238.07		43.14653

				238.09		43.08882

				238.11		43.04265

				238.14		43.01379

				238.16		42.97339

				238.18		42.90991

				238.2		42.85797

				238.22		42.81757

				238.24		42.75985

				238.26		42.6906

				238.28		42.6502

				238.3		42.6098

				238.32		42.55786

				238.35		42.50592

				238.37		42.49437

				238.39		42.43089

				238.41		42.39626

				238.43		42.33855

				238.45		42.31546

				238.47		42.24043

				238.49		42.20003

				238.51		42.15386

				238.53		42.10192

				238.56		42.03844

				238.58		42.00958

				238.6		41.94032

				238.62		41.88838

				238.64		41.84798

				238.66		41.79027

				238.68		41.70947

				238.7		41.7037

				238.72		41.64021

				238.74		41.57673

				238.77		41.53056

				238.79		41.5017

				238.81		41.43822

				238.83		41.38628

				238.85		41.34011

				238.87		41.29393

				238.89		41.23045

				238.91		41.18428

				238.93		41.14388

				238.95		41.10348

				238.98		41.05154

				239		41.02845

				239.02		40.97651

				239.04		40.91303

				239.06		40.86686

				239.08		40.82068

				239.1		40.76297

				239.12		40.69949

				239.14		40.65909

				239.16		40.61292

				239.19		40.54366

				239.21		40.50903

				239.23		40.46863

				239.25		40.41669

				239.27		40.33012

				239.29		40.33589

				239.31		40.25509

				239.33		40.19738

				239.35		40.12235

				239.37		40.12812

				239.4		40.03001

				239.42		39.99538

				239.44		39.94921

				239.46		39.92613

				239.48		39.84533

				239.5		39.79339

				239.52		39.75299

				239.54		39.67219

				239.56		39.6087

				239.58		39.5683

				239.61		39.51636

				239.63		39.42402

				239.65		39.40093

				239.67		39.34322

				239.69		39.28551

				239.71		39.22779

				239.73		39.21048

				239.75		39.13545

				239.77		39.09505

				239.79		39.03734

				239.82		38.99117

				239.84		38.92769

				239.86		38.91037

				239.88		38.84112

				239.9		38.80649

				239.92		38.75454

				239.94		38.70837

				239.96		38.65643

				239.98		38.59872

				240		38.56986

				240.03		38.51792

				240.05		38.46598

				240.07		38.39672

				240.09		38.37941

				240.11		38.28707

				240.13		38.24667

				240.15		38.18895

				240.17		38.15433

				240.19		38.0793

				240.21		38.04467

				240.24		37.98696

				240.26		37.93501

				240.28		37.8773

				240.3		37.8369

				240.32		37.79073

				240.34		37.72725

				240.36		37.70416

				240.38		37.65222

				240.4		37.60028

				240.42		37.53102

				240.45		37.51948

				240.47		37.42714

				240.49		37.36942

				240.51		37.31748

				240.53		37.28862

				240.55		37.19628

				240.57		37.16166

				240.59		37.11548

				240.61		37.052

				240.63		36.9712

				240.66		36.92503

				240.68		36.87309

				240.7		36.8096

				240.72		36.76343

				240.74		36.73458

				240.76		36.65955

				240.78		36.60761

				240.8		36.55566

				240.82		36.50372

				240.84		36.45178

				240.87		36.41715

				240.89		36.35944

				240.91		36.29595

				240.93		36.24978

				240.95		36.19207

				240.97		36.12281

				240.99		36.0651

				241.01		36.04202

				241.03		35.97276

				241.05		35.91505

				241.08		35.87465

				241.1		35.8227

				241.12		35.74768

				241.14		35.68419

				241.16		35.64956

				241.18		35.57454

				241.2		35.53414

				241.22		35.47642

				241.24		35.4418

				241.26		35.361

				241.29		35.33791

				241.31		35.29174

				241.33		35.23403

				241.35		35.16477

				241.37		35.1186

				241.39		35.06089

				241.41		34.9974

				241.43		34.93392

				241.45		34.90506

				241.47		34.86466

				241.5		34.80118

				241.52		34.74924

				241.54		34.70884

				241.56		34.62227

				241.58		34.57032

				241.6		34.52415

				241.62		34.46067

				241.64		34.40295

				241.66		34.36833

				241.68		34.28176

				241.71		34.22981

				241.73		34.1721

				241.75		34.12016

				241.77		34.06822

				241.79		34.03359

				241.81		33.99319

				241.83		33.94125

				241.85		33.88353

				241.87		33.82582

				241.89		33.79119

				241.92		33.71617

				241.94		33.64691

				241.96		33.61805

				241.98		33.5488

				242		33.47954

				242.02		33.43337

				242.04		33.41606

				242.06		33.33526

				242.08		33.29486

				242.1		33.23137

				242.13		33.16789

				242.15		33.09286

				242.17		33.04092

				242.19		32.97743

				242.21		32.93703

				242.23		32.89664

				242.25		32.85046

				242.27		32.78121

				242.29		32.7235

				242.31		32.69464

				242.34		32.61961

				242.36		32.55035

				242.38		32.5215

				242.4		32.46956

				242.42		32.38876

				242.44		32.34259

				242.46		32.30219

				242.48		32.23293

				242.5		32.18099

				242.52		32.1175

				242.54		32.05979

				242.57		31.97899

				242.59		31.92705

				242.61		31.86934

				242.63		31.81162

				242.65		31.74814

				242.67		31.71351

				242.69		31.66157

				242.71		31.59808

				242.73		31.54614

				242.75		31.4942

				242.78		31.43072

				242.8		31.36723

				242.82		31.32683

				242.84		31.26912

				242.86		31.19409

				242.88		31.14215

				242.9		31.08443

				242.92		31.01518

				242.94		30.96324

				242.96		30.94015

				242.99		30.87667

				243.01		30.81318

				243.03		30.77855

				243.05		30.69775

				243.07		30.63427

				243.09		30.5881

				243.11		30.53039

				243.13		30.47267

				243.15		30.44382

				243.17		30.39187

				243.2		30.33416

				243.22		30.28222

				243.24		30.21296

				243.26		30.15525

				243.28		30.08599

				243.3		30.05714

				243.32		29.98211

				243.34		29.91862

				243.36		29.85514

				243.39		29.83205

				243.41		29.71086

				243.43		29.682

				243.45		29.62429

				243.47		29.57812

				243.49		29.50309

				243.51		29.47423

				243.53		29.41652

				243.55		29.34726

				243.57		29.30686

				243.6		29.24338

				243.62		29.17412

				243.64		29.11064

				243.66		29.07024

				243.68		28.98944

				243.7		28.93173

				243.72		28.8971

				243.74		28.8567

				243.76		28.79321

				243.78		28.72396

				243.81		28.6951

				243.83		28.63162

				243.85		28.55082

				243.87		28.48733

				243.89		28.43539

				243.91		28.34882

				243.93		28.28534

				243.95		28.22185

				243.97		28.16991

				243.99		28.11797

				244.02		28.06025

				244.04		28.00831

				244.06		27.98523

				244.08		27.91597

				244.1		27.86403

				244.12		27.789

				244.14		27.73706

				244.16		27.63894

				244.18		27.59277

				244.2		27.5062

				244.22		27.48889

				244.25		27.40809

				244.27		27.36769

				244.29		27.30998

				244.31		27.27535

				244.33		27.21187

				244.35		27.17147

				244.37		27.11375

				244.39		27.05604

				244.41		27.01564

				244.43		26.92907

				244.46		26.89444

				244.48		26.82519

				244.5		26.76747

				244.52		26.68667

				244.54		26.63473

				244.56		26.53662

				244.58		26.49045

				244.6		26.42696

				244.62		26.37502

				244.64		26.30577

				244.67		26.28268

				244.69		26.22497

				244.71		26.15571

				244.73		26.098

				244.75		26.05183

				244.77		25.98834

				244.79		25.92486

				244.81		25.87292

				244.83		25.8152

				244.85		25.75172

				244.88		25.66515

				244.9		25.6132

				244.92		25.56126

				244.94		25.49201

				244.96		25.42852

				244.98		25.40544

				245		25.31887

				245.02		25.26115

				245.04		25.20921

				245.06		25.14573

				245.09		25.0707

				245.11		25.0303

				245.13		24.97836

				245.15		24.9091

				245.17		24.88024

				245.19		24.81676

				245.21		24.76482

				245.23		24.7071

				245.25		24.65516

				245.27		24.57436

				245.29		24.52242

				245.32		24.45894

				245.34		24.39545

				245.36		24.33774

				245.38		24.2858

				245.4		24.205

				245.42		24.14728

				245.44		24.08957

				245.46		24.02032

				245.48		23.9626

				245.5		23.91643

				245.53		23.85295

				245.55		23.78946

				245.57		23.73175

				245.59		23.66826

				245.61		23.61632

				245.63		23.54707

				245.65		23.48935

				245.67		23.43164

				245.69		23.36238

				245.71		23.29313

				245.74		23.24118

				245.76		23.18347

				245.78		23.11999

				245.8		23.06804

				245.82		23.00456

				245.84		22.92376

				245.86		22.8545

				245.88		22.80833

				245.9		22.74485

				245.92		22.68136

				245.94		22.64674

				245.97		22.58902

				245.99		22.52554

				246.01		22.46205

				246.03		22.41011

				246.05		22.35817

				246.07		22.28314

				246.09		22.21389

				246.11		22.15617

				246.13		22.08115

				246.15		22.0292

				246.18		21.97726

				246.2		21.91955

				246.22		21.85029

				246.24		21.79835

				246.26		21.73486

				246.28		21.67715

				246.3		21.61367

				246.32		21.57327

				246.34		21.50978

				246.36		21.42898

				246.39		21.37704

				246.41		21.30779

				246.43		21.2443

				246.45		21.18659

				246.47		21.13465

				246.49		21.05962

				246.51		21.03653

				246.53		20.96151

				246.55		20.88071

				246.57		20.82876

				246.59		20.76528

				246.62		20.68448

				246.64		20.62677

				246.66		20.59214

				246.68		20.51134

				246.7		20.4594

				246.72		20.39014

				246.74		20.3382

				246.76		20.26317

				246.78		20.19969

				246.8		20.14197

				246.83		20.09003

				246.85		20.03232

				246.87		19.98038

				246.89		19.93421

				246.91		19.84764

				246.93		19.79569

				246.95		19.72067

				246.97		19.6341

				246.99		19.57061

				247.01		19.54753

				247.04		19.48404

				247.06		19.42056

				247.08		19.36862

				247.1		19.32822

				247.12		19.25319

				247.14		19.17816

				247.16		19.12622

				247.18		19.07428

				247.2		18.98194

				247.22		18.94731

				247.24		18.88959

				247.27		18.83765

				247.29		18.76262

				247.31		18.72223

				247.33		18.61834

				247.35		18.56063

				247.37		18.4856

				247.39		18.43366

				247.41		18.34132

				247.43		18.27783

				247.45		18.22012

				247.48		18.15086

				247.5		18.07006

				247.52		18.04698

				247.54		18.01235

				247.56		17.92001

				247.58		17.86807

				247.6		17.84498

				247.62		17.75264

				247.64		17.68916

				247.66		17.66607

				247.69		17.60836

				247.71		17.51602

				247.73		17.4987

				247.75		17.4179

				247.77		17.34288

				247.79		17.27362

				247.81		17.22168

				247.83		17.12356

				247.85		17.04854

				247.87		16.99082

				247.89		16.93888

				247.92		16.85231

				247.94		16.78306

				247.96		16.75997

				247.98		16.6734

				248		16.5926

				248.02		16.58683

				248.04		16.52335

				248.06		16.46563

				248.08		16.3906

				248.1		16.36752

				248.13		16.25786

				248.15		16.21746

				248.17		16.14821

				248.19		16.09627

				248.21		16.00392

				248.23		15.95775

				248.25		15.87118

				248.27		15.79616

				248.29		15.74999

				248.31		15.6865

				248.34		15.59416

				248.36		15.55376

				248.38		15.50182

				248.4		15.42679

				248.42		15.36908

				248.44		15.32868

				248.46		15.23634

				248.48		15.16131

				248.5		15.12091

				248.52		15.05165

				248.55		14.95931

				248.57		14.94777

				248.59		14.89006

				248.61		14.8208

				248.63		14.75154

				248.65		14.72269

				248.67		14.64766

				248.69		14.5784

				248.71		14.50915

				248.73		14.45143

				248.76		14.35909

				248.78		14.27829

				248.8		14.22635

				248.82		14.17441

				248.84		14.09938

				248.86		14.08207

				248.88		14.01858

				248.9		13.94933

				248.92		13.8743

				248.94		13.83967

				248.97		13.74733

				248.99		13.67807

				249.01		13.61459

				249.03		13.57996

				249.05		13.49339

				249.07		13.42991

				249.09		13.38951

				249.11		13.32602

				249.13		13.22791

				249.15		13.17597

				249.17		13.14134

				249.2		13.02014

				249.22		12.98551

				249.24		12.90472

				249.26		12.85854

				249.28		12.75466

				249.3		12.74312

				249.32		12.63346

				249.34		12.58729

				249.36		12.52381

				249.38		12.48341

				249.41		12.40261

				249.43		12.35644

				249.45		12.33335

				249.47		12.25255

				249.49		12.19484

				249.51		12.13713

				249.53		12.09096

				249.55		11.9813

				249.57		11.9409

				249.59		11.87742

				249.62		11.80816

				249.64		11.7389

				249.66		11.72159

				249.68		11.62348

				249.7		11.55999

				249.72		11.49074

				249.74		11.45034

				249.76		11.3176

				249.78		11.28874

				249.8		11.23103

				249.82		11.16754

				249.85		11.0752

				249.87		11.05212

				249.89		10.98863

				249.91		10.89629

				249.93		10.85589

				249.95		10.80972

				249.97		10.73469

				249.99		10.64812

				250.01		10.63081

				250.03		10.56155

				250.06		10.4923

				250.08		10.44035

				250.1		10.39995

				250.12		10.31916

				250.14		10.26144

				250.16		10.19796

				250.18		10.12293

				250.2		10.05944

				250.22		9.990189

				250.24		9.90939

				250.27		9.851677

				250.29		9.811277

				250.31		9.730478

				250.33		9.690079

				250.35		9.632366

				250.37		9.574652

				250.39		9.47654

				250.41		9.441911

				250.43		9.384198

				250.45		9.332256

				250.48		9.257229

				250.5		9.239915

				250.52		9.170659

				250.54		9.084088

				250.56		9.014832

				250.58		8.985976

				250.6		8.887863

				250.62		8.830149

				250.64		8.772436

				250.66		8.737808

				250.68		8.633924

				250.71		8.593525

				250.73		8.535811

				250.75		8.466555

				250.77		8.379985

				250.79		8.362671

				250.81		8.281872

				250.83		8.201073

				250.85		8.154903

				250.87		8.097189

				250.89		8.016391

				250.92		7.981763

				250.94		7.958677

				250.96		7.895192

				250.98		7.84325

				251		7.79708

				251.02		7.750909

				251.04		7.658568

				251.06		7.612397

				251.08		7.554683

				251.1		7.479656

				251.13		7.393086

				251.15		7.358458

				251.17		7.277659

				251.19		7.202632

				251.21		7.162232

				251.23		7.11029

				251.25		7.02372

				251.27		6.977549

				251.29		6.93715

				251.31		6.85058

				251.33		6.76401

				251.36		6.729382

				251.38		6.660126

				251.4		6.579327

				251.42		6.533156

				251.44		6.498528

				251.46		6.423501

				251.48		6.348473

				251.5		6.325388

				251.52		6.273446

				251.54		6.198419

				251.56		6.146477

				251.59		6.106077

				251.61		6.013736

				251.63		5.950251

				251.65		5.90408

				251.67		5.834824

				251.69		5.77134

				251.71		5.719397

				251.73		5.661684

				251.75		5.598199

				251.77		5.552029

				251.8		5.500087

				251.82		5.436602

				251.84		5.38466

				251.86		5.326946

				251.88		5.269233

				251.9		5.188434

				251.92		5.142264

				251.94		5.090321

				251.96		5.009523

				251.98		4.957581

				252		4.917181

				252.03		4.865239

				252.05		4.790212

				252.07		4.755584

				252.09		4.692099

				252.11		4.622843

				252.13		4.559358

				252.15		4.52473

				252.17		4.461245

				252.19		4.409303

				252.21		4.368904

				252.23		4.293877

				252.26		4.207307

				252.28		4.143822

				252.3		4.086108

				252.32		4.022624

				252.34		3.970682

				252.36		3.941825

				252.38		3.901426

				252.4		3.832169

				252.42		3.79177

				252.44		3.734057

				252.47		3.670572

				252.49		3.607087

				252.51		3.595545

				252.53		3.503203

				252.55		3.457032

				252.57		3.416633

				252.59		3.387776

				252.61		3.289664

				252.63		3.27235

				252.65		3.226179

				252.67		3.151151

				252.7		3.099209

				252.72		3.064581

				252.74		3.006868

				252.76		2.949154

				252.78		2.93184

				252.8		2.88567

				252.82		2.833728

				252.84		2.781786

				252.86		2.752929

				252.88		2.683673

				252.91		2.649045

				252.93		2.620188

				252.95		2.614417

				252.97		2.556703

				252.99		2.539389

				253.01		2.49899

				253.03		2.452819

				253.05		2.395106

				253.07		2.366249

				253.09		2.331621

				253.11		2.291222

				253.14		2.262365

				253.16		2.216194

				253.18		2.204652

				253.2		2.164252

				253.22		2.158481

				253.24		2.135396

				253.26		2.123853

				253.28		2.089225

				253.3		2.089225

				253.32		2.043054

				253.35		2.043054

				253.37		2.037283

				253.39		2.019969

				253.41		2.002655

				253.43		2.014197

				253.45		1.985341

				253.47		1.962255

				253.49		1.968027

				253.51		1.944941

				253.53		1.944941

				253.55		1.910313

				253.58		1.950713

				253.6		1.904542

				253.62		1.898771

				253.64		1.881457

				253.66		1.881457

				253.68		1.823743

				253.7		1.835286

				253.72		1.823743

				253.74		1.806429

				253.76		1.812201

				253.79		1.806429

				253.81		1.789115

				253.83		1.777573

				253.85		1.789115

				253.87		1.777573

				253.89		1.760259

				253.91		1.783344

				253.93		1.771801

				253.95		1.760259

				253.97		1.76603

				253.99		1.777573

				254.02		1.777573

				254.04		1.754487

				254.06		1.754487

				254.08		1.760259

				254.1		1.754487

				254.12		1.748716

				254.14		1.742945

				254.16		1.737173

				254.18		1.737173

				254.2		1.742945

				254.23		1.731402

				254.25		1.731402

				254.27		1.725631

				254.29		1.725631

				254.31		1.719859

				254.33		1.725631

				254.35		1.725631

				254.37		1.719859

				254.39		1.725631

				254.41		1.719859

				254.43		1.719859

				254.46		1.714088

				254.48		1.714088

				254.5		1.708317

				254.52		1.714088

				254.54		1.708317

				254.56		1.708317

				254.58		1.708317

				254.6		1.708317

				254.62		1.702545

				254.64		1.708317

				254.66		1.702545

				254.69		1.702545

				254.71		1.702545

				254.73		1.702545

				254.75		1.696774

				254.77		1.691002

				254.79		1.691002

				254.81		1.691002

				254.83		1.691002

				254.85		1.685231

				254.87		1.685231

				254.89		1.685231

				254.92		1.685231

				254.94		1.685231

				254.96		1.67946

				254.98		1.67946

				255		1.67946

				255.02		1.67946

				255.04		1.67946

				255.06		1.673688

				255.08		1.673688

				255.1		1.673688

				255.12		1.667917

				255.15		1.667917

				255.17		1.667917

				255.19		1.667917

				255.21		1.662146

				255.23		1.662146

				255.25		1.662146

				255.27		1.662146

				255.29		1.662146

				255.31		1.662146

				255.33		1.662146

				255.35		1.656374

				255.38		1.656374

				255.4		1.656374

				255.42		1.656374

				255.44		1.656374

				255.46		1.656374

				255.48		1.656374

				255.5		1.656374

				255.52		1.650603

				255.54		1.650603

				255.56		1.650603

				255.58		1.650603

				255.61		1.650603

				255.63		1.644832

				255.65		1.644832

				255.67		1.644832

				255.69		1.644832

				255.71		1.644832

				255.73		1.644832

				255.75		1.644832

				255.77		1.63906

				255.79		1.63906

				255.81		1.63906

				255.84		1.63906

				255.86		1.63906

				255.88		1.633289

				255.9		1.633289

				255.92		1.633289

				255.94		1.633289

				255.96		1.633289

				255.98		1.633289

				256		1.633289

				256.02		1.633289

				256.04		1.633289

				256.06		1.633289

				256.09		1.627518

				256.11		1.627518

				256.13		1.627518

				256.15		1.627518

				256.17		1.627518

				256.19		1.627518

				256.21		1.627518

				256.23		1.627518

				256.25		1.627518

				256.27		1.621746

				256.29		1.621746

				256.32		1.621746

				256.34		1.621746

				256.36		1.621746

				256.38		1.621746

				256.4		1.621746

				256.42		1.621746

				256.44		1.621746

				256.46		1.621746

				256.48		1.621746

				256.5		1.615975

				256.52		1.615975

				256.55		1.615975

				256.57		1.615975

				256.59		1.615975

				256.61		1.615975

				256.63		1.615975

				256.65		1.615975

				256.67		1.610204

				256.69		1.610204

				256.71		1.610204

				256.73		1.610204

				256.75		1.610204

				256.77		1.610204

				256.8		1.610204

				256.82		1.610204

				256.84		1.610204

				256.86		1.604432

				256.88		1.604432

				256.9		1.604432

				256.92		1.604432

				256.94		1.604432

				256.96		1.604432

				256.98		1.604432

				257		1.604432

				257.03		1.598661

				257.05		1.598661

				257.07		1.598661

				257.09		1.598661

				257.11		1.598661

				257.13		1.598661

				257.15		1.598661

				257.17		1.59289

				257.19		1.59289

				257.21		1.59289

				257.23		1.59289

				257.26		1.59289

				257.28		1.59289

				257.3		1.59289

				257.32		1.59289

				257.34		1.59289

				257.36		1.59289

				257.38		1.587118

				257.4		1.587118

				257.42		1.587118

				257.44		1.587118

				257.46		1.587118

				257.49		1.587118

				257.51		1.587118

				257.53		1.587118

				257.55		1.581347

				257.57		1.581347

				257.59		1.581347

				257.61		1.581347

				257.63		1.581347

				257.65		1.581347

				257.67		1.581347

				257.69		1.575576

				257.72		1.581347

				257.74		1.575576

				257.76		1.575576

				257.78		1.575576

				257.8		1.575576

				257.82		1.575576

				257.84		1.575576

				257.86		1.575576

				257.88		1.575576

				257.9		1.575576

				257.92		1.569804

				257.95		1.569804

				257.97		1.569804

				257.99		1.569804

				258.01		1.569804

				258.03		1.569804

				258.05		1.569804

				258.07		1.569804

				258.09		1.569804

				258.11		1.569804

				258.13		1.569804

				258.15		1.569804

				258.18		1.564033

				258.2		1.564033

				258.22		1.564033

				258.24		1.564033

				258.26		1.564033

				258.28		1.564033

				258.3		1.564033

				258.32		1.564033

				258.34		1.564033

				258.36		1.564033

				258.38		1.558262

				258.41		1.558262

				258.43		1.558262

				258.45		1.558262

				258.47		1.558262

				258.49		1.558262

				258.51		1.558262

				258.53		1.558262

				258.55		1.558262

				258.57		1.558262

				258.59		1.558262

				258.61		1.558262

				258.64		1.558262

				258.66		1.55249

				258.68		1.55249

				258.7		1.55249

				258.72		1.55249

				258.74		1.55249

				258.76		1.55249

				258.78		1.55249

				258.8		1.55249

				258.82		1.55249

				258.84		1.55249

				258.87		1.55249

				258.89		1.55249

				258.91		1.55249

				258.93		1.55249

				258.95		1.546719

				258.97		1.55249

				258.99		1.546719

				259.01		1.546719

				259.03		1.546719

				259.05		1.546719

				259.07		1.546719

				259.09		1.546719

				259.12		1.546719

				259.14		1.546719

				259.16		1.546719

				259.18		1.546719

				259.2		1.546719

				259.22		1.546719

				259.24		1.546719

				259.26		1.546719

				259.28		1.546719

				259.3		1.540948

				259.32		1.540948

				259.35		1.546719

				259.37		1.540948

				259.39		1.540948

				259.41		1.540948

				259.43		1.540948

				259.45		1.540948

				259.47		1.540948

				259.49		1.540948

				259.51		1.540948

				259.53		1.540948

				259.55		1.540948

				259.58		1.540948

				259.6		1.540948

				259.62		1.540948

				259.64		1.540948

				259.66		1.540948

				259.68		1.540948

				259.7		1.540948

				259.72		1.540948

				259.74		1.540948

				259.76		1.540948

				259.78		1.540948

				259.8		1.540948

				259.83		1.540948

				259.85		1.540948

				259.87		1.540948

				259.89		1.540948

				259.91		1.540948

				259.93		1.540948

				259.95		1.540948

				259.97		1.540948

				259.99		1.540948

				260.01		1.535176

				260.03		1.535176

				260.06		1.535176

				260.08		1.535176

				260.1		1.535176

				260.12		1.535176

				260.14		1.535176

				260.16		1.535176

				260.18		1.535176

				260.2		1.535176

				260.22		1.535176

				260.24		1.535176

				260.26		1.535176

				260.28		1.535176

				260.31		1.535176

				260.33		1.535176

				260.35		1.535176

				260.37		1.535176

				260.39		1.535176

				260.41		1.535176

				260.43		1.535176

				260.45		1.535176

				260.47		1.535176

				260.49		1.535176

				260.51		1.535176

				260.54		1.535176

				260.56		1.535176

				260.58		1.535176

				260.6		1.535176

				260.62		1.535176

				260.64		1.535176

				260.66		1.535176

				260.68		1.535176

				260.7		1.529405

				260.72		1.529405

				260.74		1.529405

				260.77		1.529405

				260.79		1.529405

				260.81		1.529405

				260.83		1.529405

				260.85		1.529405

				260.87		1.529405

				260.89		1.529405

				260.91		1.529405

				260.93		1.529405

				260.95		1.529405

				260.97		1.529405

				260.99		1.529405

				261.02		1.529405

				261.04		1.529405

				261.06		1.529405

				261.08		1.529405

				261.1		1.529405

				261.12		1.529405

				261.14		1.529405

				261.16		1.529405

				261.18		1.529405

				261.2		1.529405

				261.22		1.529405

				261.25		1.529405

				261.27		1.529405

				261.29		1.529405

				261.31		1.529405

				261.33		1.529405

				261.35		1.529405

				261.37		1.529405

				261.39		1.529405

				261.41		1.529405

				261.43		1.529405

				261.45		1.529405

				261.48		1.529405

				261.5		1.529405

				261.52		1.529405

				261.54		1.529405

				261.56		1.529405

				261.58		1.529405

				261.6		1.529405

				261.62		1.529405

				261.64		1.529405

				261.66		1.529405

				261.68		1.529405

				261.71		1.529405

				261.73		1.529405

				261.75		1.529405

				261.77		1.529405

				261.79		1.529405

				261.81		1.529405

				261.83		1.529405

				261.85		1.529405

				261.87		1.529405

				261.89		1.523634

				261.91		1.529405

				261.94		1.523634

				261.96		1.523634

				261.98		1.529405

				262		1.529405

				262.02		1.529405

				262.04		1.529405

				262.06		1.523634

				262.08		1.523634

				262.1		1.523634

				262.12		1.523634

				262.14		1.523634

				262.17		1.523634

				262.19		1.523634

				262.21		1.523634

				262.23		1.523634

				262.25		1.523634

				262.27		1.523634

				262.29		1.523634

				262.31		1.523634

				262.33		1.523634

				262.35		1.523634

				262.37		1.523634

				262.39		1.523634

				262.42		1.523634

				262.44		1.523634

				262.46		1.523634

				262.48		1.517862

				262.5		1.523634

				262.52		1.523634

				262.54		1.523634

				262.56		1.523634

				262.58		1.523634

				262.6		1.523634

				262.62		1.523634

				262.65		1.523634

				262.67		1.523634

				262.69		1.523634

				262.71		1.517862

				262.73		1.517862

				262.75		1.523634

				262.77		1.523634

				262.79		1.523634

				262.81		1.517862

				262.83		1.517862

				262.85		1.517862

				262.88		1.517862

				262.9		1.517862

				262.92		1.517862

				262.94		1.517862

				262.96		1.517862

				262.98		1.517862

				263		1.517862

				263.02		1.517862

				263.04		1.517862

				263.06		1.517862

				263.08		1.517862

				263.1		1.517862

				263.13		1.517862

				263.15		1.517862

				263.17		1.517862

				263.19		1.517862

				263.21		1.517862

				263.23		1.512091

				263.25		1.512091

				263.27		1.512091

				263.29		1.512091

				263.31		1.512091

				263.33		1.512091

				263.36		1.512091

				263.38		1.512091

				263.4		1.512091

				263.42		1.512091

				263.44		1.512091

				263.46		1.512091

				263.48		1.512091

				263.5		1.512091

				263.52		1.512091

				263.54		1.512091

				263.56		1.512091

				263.59		1.50632

				263.61		1.512091

				263.63		1.50632

				263.65		1.50632

				263.67		1.50632

				263.69		1.50632

				263.71		1.50632

				263.73		1.50632

				263.75		1.50632

				263.77		1.50632

				263.79		1.50632

				263.81		1.50632

				263.84		1.50632

				263.86		1.50632

				263.88		1.50632

				263.9		1.50632

				263.92		1.50632

				263.94		1.50632

				263.96		1.50632

				263.98		1.50632

				264		1.50632

				264.02		1.50632

				264.04		1.500548

				264.07		1.500548

				264.09		1.500548

				264.11		1.500548

				264.13		1.500548

				264.15		1.500548

				264.17		1.500548

				264.19		1.500548

				264.21		1.500548

				264.23		1.500548

				264.25		1.500548

				264.27		1.500548

				264.29		1.500548

				264.32		1.500548

				264.34		1.500548

				264.36		1.500548

				264.38		1.500548

				264.4		1.500548

				264.42		1.500548

				264.44		1.500548

				264.46		1.500548

				264.48		1.500548

				264.5		1.500548

				264.52		1.500548

				264.54		1.500548

				264.57		1.500548

				264.59		1.500548

				264.61		1.500548

				264.63		1.500548

				264.65		1.494777

				264.67		1.500548

				264.69		1.494777

				264.71		1.494777

				264.73		1.494777

				264.75		1.494777

				264.77		1.494777

				264.8		1.494777

				264.82		1.494777

				264.84		1.494777

				264.86		1.494777

				264.88		1.494777

				264.9		1.494777

				264.92		1.494777

				264.94		1.494777

				264.96		1.494777

				264.98		1.489006

				265		1.489006

				265.02		1.489006

				265.04		1.483234

				265.07		1.483234

				265.09		1.483234

				265.11		1.483234

				265.13		1.483234

				265.15		1.477463

				265.17		1.477463

				265.19		1.477463

				265.21		1.477463

				265.23		1.477463

				265.25		1.477463

				265.27		1.477463

				265.29		1.477463

				265.32		1.477463

				265.34		1.477463

				265.36		1.477463

				265.38		1.471692

				265.4		1.471692

				265.42		1.471692

				265.44		1.471692

				265.46		1.471692

				265.48		1.471692

				265.5		1.471692

				265.52		1.471692

				265.55		1.471692

				265.57		1.471692

				265.59		1.46592

				265.61		1.471692

				265.63		1.46592

				265.65		1.46592

				265.67		1.46592

				265.69		1.46592

				265.71		1.46592

				265.73		1.46592

				265.75		1.46592

				265.77		1.460149

				265.8		1.460149

				265.82		1.460149

				265.84		1.460149

				265.86		1.460149

				265.88		1.460149

				265.9		1.460149

				265.92		1.460149

				265.94		1.460149

				265.96		1.460149

				265.98		1.460149

				266		1.460149

				266.02		1.460149

				266.05		1.460149

				266.07		1.460149

				266.09		1.460149

				266.11		1.460149

				266.13		1.460149

				266.15		1.460149

				266.17		1.460149

				266.19		1.460149

				266.21		1.460149

				266.23		1.460149

				266.25		1.460149

				266.27		1.460149

				266.3		1.460149

				266.32		1.460149

				266.34		1.460149

				266.36		1.460149

				266.38		1.460149

				266.4		1.460149

				266.42		1.460149

				266.44		1.460149

				266.46		1.460149

				266.48		1.460149

				266.5		1.460149

				266.52		1.460149

				266.55		1.460149

				266.57		1.460149

				266.59		1.454378

				266.61		1.454378

				266.63		1.454378

				266.65		1.454378

				266.67		1.454378

				266.69		1.454378

				266.71		1.460149

				266.73		1.460149

				266.75		1.454378

				266.77		1.454378

				266.8		1.460149

				266.82		1.460149

				266.84		1.460149

				266.86		1.460149

				266.88		1.454378

				266.9		1.454378

				266.92		1.454378

				266.94		1.454378

				266.96		1.460149

				266.98		1.460149

				267		1.460149

				267.02		1.460149

				267.05		1.46592

				267.07		1.46592

				267.09		1.46592

				267.11		1.46592

				267.13		1.46592

				267.15		1.46592

				267.17		1.46592

				267.19		1.46592

				267.21		1.46592

				267.23		1.46592

				267.25		1.46592

				267.27		1.471692

				267.3		1.471692

				267.32		1.46592

				267.34		1.471692

				267.36		1.471692

				267.38		1.471692

				267.4		1.471692

				267.42		1.471692

				267.44		1.471692

				267.46		1.471692

				267.48		1.471692

				267.5		1.471692

				267.52		1.471692

				267.55		1.471692

				267.57		1.471692

				267.59		1.471692

				267.61		1.471692

				267.63		1.471692

				267.65		1.471692

				267.67		1.471692

				267.69		1.471692

				267.71		1.471692

				267.73		1.471692

				267.75		1.471692

				267.78		1.471692

				267.8		1.471692

				267.82		1.471692

				267.84		1.471692

				267.86		1.471692

				267.88		1.471692

				267.9		1.471692

				267.92		1.471692

				267.94		1.471692

				267.96		1.477463

				267.98		1.477463

				268		1.477463

				268.03		1.471692

				268.05		1.471692

				268.07		1.471692

				268.09		1.471692

				268.11		1.477463

				268.13		1.477463

				268.15		1.477463

				268.17		1.477463

				268.19		1.477463

				268.21		1.477463

				268.23		1.477463

				268.25		1.477463

				268.28		1.477463

				268.3		1.477463

				268.32		1.471692

				268.34		1.477463

				268.36		1.471692

				268.38		1.477463

				268.4		1.471692

				268.42		1.471692

				268.44		1.471692

				268.46		1.471692

				268.48		1.471692

				268.51		1.471692

				268.53		1.471692

				268.55		1.471692

				268.57		1.471692

				268.59		1.471692

				268.61		1.471692

				268.63		1.471692

				268.65		1.471692

				268.67		1.471692

				268.69		1.471692

				268.71		1.471692

				268.73		1.471692

				268.76		1.471692

				268.78		1.471692

				268.8		1.471692

				268.82		1.471692

				268.84		1.471692

				268.86		1.471692

				268.88		1.471692

				268.9		1.471692

				268.92		1.471692

				268.94		1.471692

				268.96		1.471692

				268.98		1.471692

				269.01		1.471692

				269.03		1.46592

				269.05		1.471692

				269.07		1.471692

				269.09		1.471692

				269.11		1.471692

				269.13		1.471692

				269.15		1.471692

				269.17		1.471692

				269.19		1.471692

				269.21		1.471692

				269.24		1.471692

				269.26		1.471692

				269.28		1.471692

				269.3		1.471692

				269.32		1.471692

				269.34		1.471692

				269.36		1.471692

				269.38		1.471692

				269.4		1.471692

				269.42		1.471692

				269.44		1.471692

				269.46		1.471692

				269.49		1.471692

				269.51		1.471692

				269.53		1.471692

				269.55		1.471692

				269.57		1.471692

				269.59		1.46592

				269.61		1.471692

				269.63		1.471692

				269.65		1.46592

				269.67		1.46592

				269.69		1.46592

				269.72		1.471692

				269.74		1.46592

				269.76		1.46592

				269.78		1.46592

				269.8		1.46592

				269.82		1.46592

				269.84		1.46592

				269.86		1.46592

				269.88		1.471692

				269.9		1.46592

				269.92		1.46592

				269.94		1.46592

				269.97		1.46592

				269.99		1.46592

				270.01		1.46592

				270.03		1.46592

				270.05		1.46592

				270.07		1.46592

				270.09		1.46592

				270.11		1.46592

				270.13		1.46592

				270.15		1.46592

				270.17		1.46592

				270.19		1.46592

				270.22		1.46592

				270.24		1.46592

				270.26		1.46592

				270.28		1.46592

				270.3		1.46592

				270.32		1.46592

				270.34		1.46592

				270.36		1.46592

				270.38		1.46592

				270.4		1.46592

				270.42		1.46592

				270.45		1.46592

				270.47		1.46592

				270.49		1.46592

				270.51		1.46592

				270.53		1.46592

				270.55		1.46592

				270.57		1.46592

				270.59		1.46592

				270.61		1.46592

				270.63		1.46592

				270.65		1.46592

				270.68		1.46592

				270.7		1.46592

				270.72		1.46592

				270.74		1.46592

				270.76		1.46592

				270.78		1.46592

				270.8		1.46592

				270.82		1.46592

				270.84		1.46592

				270.86		1.46592

				270.88		1.46592

				270.9		1.46592

				270.93		1.46592

				270.95		1.46592

				270.97		1.46592

				270.99		1.46592

				271.01		1.46592

				271.03		1.46592

				271.05		1.46592

				271.07		1.46592

				271.09		1.46592

				271.11		1.46592

				271.13		1.46592

				271.16		1.46592

				271.18		1.46592

				271.2		1.46592

				271.22		1.46592

				271.24		1.46592

				271.26		1.46592

				271.28		1.46592

				271.3		1.46592

				271.32		1.46592

				271.34		1.46592

				271.36		1.460149

				271.39		1.460149

				271.41		1.460149

				271.43		1.460149

				271.45		1.460149

				271.47		1.46592

				271.49		1.46592

				271.51		1.460149

				271.53		1.46592

				271.55		1.46592

				271.57		1.46592

				271.59		1.46592

				271.62		1.46592

				271.64		1.46592

				271.66		1.46592

				271.68		1.460149

				271.7		1.460149

				271.72		1.46592

				271.74		1.460149

				271.76		1.460149

				271.78		1.460149

				271.8		1.460149

				271.82		1.460149

				271.85		1.460149

				271.87		1.460149

				271.89		1.460149

				271.91		1.460149

				271.93		1.460149

				271.95		1.460149

				271.97		1.460149

				271.99		1.460149

				272.01		1.460149

				272.03		1.460149

				272.05		1.460149

				272.08		1.460149

				272.1		1.460149

				272.12		1.460149

				272.14		1.460149

				272.16		1.460149

				272.18		1.460149

				272.2		1.460149

				272.22		1.460149

				272.24		1.460149

				272.26		1.454378

				272.28		1.460149

				272.3		1.454378

				272.33		1.460149

				272.35		1.454378

				272.37		1.454378

				272.39		1.454378

				272.41		1.454378

				272.43		1.454378

				272.45		1.454378

				272.47		1.454378

				272.49		1.454378

				272.51		1.454378

				272.53		1.454378

				272.56		1.454378

				272.58		1.454378

				272.6		1.454378

				272.62		1.454378

				272.64		1.454378

				272.66		1.454378

				272.68		1.448606

				272.7		1.448606

				272.72		1.448606

				272.74		1.448606

				272.76		1.448606

				272.79		1.448606

				272.81		1.448606

				272.83		1.448606

				272.85		1.448606

				272.87		1.448606

				272.89		1.448606

				272.91		1.448606

				272.93		1.448606

				272.95		1.448606

				272.97		1.448606

				272.99		1.448606

				273.02		1.448606

				273.04		1.448606

				273.06		1.448606

				273.08		1.442835

				273.1		1.442835

				273.12		1.442835

				273.14		1.442835

				273.16		1.442835

				273.18		1.442835

				273.2		1.442835

				273.22		1.442835

				273.25		1.442835

				273.27		1.442835

				273.29		1.442835

				273.31		1.442835

				273.33		1.442835

				273.35		1.442835

				273.37		1.442835

				273.39		1.442835

				273.41		1.442835

				273.43		1.442835

				273.45		1.437064

				273.48		1.437064

				273.5		1.437064

				273.52		1.437064

				273.54		1.437064

				273.56		1.437064

				273.58		1.437064

				273.6		1.437064

				273.62		1.437064

				273.64		1.437064

				273.66		1.437064

				273.68		1.431292

				273.71		1.431292

				273.73		1.431292

				273.75		1.431292

				273.77		1.437064

				273.79		1.431292

				273.81		1.431292

				273.83		1.437064

				273.85		1.437064

				273.87		1.437064

				273.89		1.437064

				273.91		1.437064

				273.94		1.431292

				273.96		1.431292

				273.98		1.431292

				274		1.431292

				274.02		1.431292

				274.04		1.431292

				274.06		1.431292

				274.08		1.431292

				274.1		1.431292

				274.12		1.431292

				274.14		1.431292

				274.17		1.431292

				274.19		1.431292

				274.21		1.431292

				274.23		1.431292

				274.25		1.431292

				274.27		1.431292

				274.29		1.431292

				274.31		1.431292

				274.33		1.431292

				274.35		1.431292

				274.37		1.431292

				274.4		1.431292

				274.42		1.431292

				274.44		1.425521

				274.46		1.431292

				274.48		1.425521

				274.5		1.431292

				274.52		1.425521

				274.54		1.425521

				274.56		1.425521

				274.58		1.425521

				274.6		1.425521

				274.63		1.425521

				274.65		1.425521

				274.67		1.425521

				274.69		1.425521

				274.71		1.425521

				274.73		1.425521

				274.75		1.425521

				274.77		1.425521

				274.79		1.425521

				274.81		1.425521

				274.83		1.425521

				274.86		1.425521

				274.88		1.425521

				274.9		1.425521

				274.92		1.425521

				274.94		1.425521

				274.96		1.425521

				274.98		1.425521

				275		1.425521

				275.02		1.425521

				275.04		1.425521

				275.06		1.425521

				275.09		1.425521

				275.11		1.425521

				275.13		1.425521

				275.15		1.425521

				275.17		1.425521

				275.19		1.425521

				275.21		1.425521

				275.23		1.425521

				275.25		1.431292

				275.27		1.425521

				275.29		1.425521

				275.32		1.425521

				275.34		1.431292

				275.36		1.425521

				275.38		1.431292

				275.4		1.431292

				275.42		1.425521

				275.44		1.425521

				275.46		1.431292

				275.48		1.425521

				275.5		1.425521

				275.53		1.425521

				275.55		1.431292

				275.57		1.425521

				275.59		1.431292

				275.61		1.431292

				275.63		1.431292

				275.65		1.431292

				275.67		1.431292

				275.69		1.431292

				275.71		1.431292

				275.73		1.431292

				275.76		1.431292

				275.78		1.431292

				275.8		1.431292

				275.82		1.431292

				275.84		1.431292

				275.86		1.431292

				275.88		1.431292

				275.9		1.431292

				275.92		1.431292

				275.94		1.431292

				275.97		1.431292

				275.99		1.431292

				276.01		1.431292

				276.03		1.431292

				276.05		1.431292

				276.07		1.431292

				276.09		1.431292

				276.11		1.431292

				276.13		1.431292

				276.15		1.431292

				276.17		1.437064

				276.2		1.437064

				276.22		1.437064

				276.24		1.437064

				276.26		1.437064

				276.28		1.437064

				276.3		1.437064

				276.32		1.437064

				276.34		1.437064

				276.36		1.437064

				276.38		1.437064

				276.41		1.437064

				276.43		1.437064

				276.45		1.437064

				276.47		1.437064

				276.49		1.437064

				276.51		1.437064

				276.53		1.437064

				276.55		1.437064

				276.57		1.437064

				276.59		1.437064

				276.62		1.437064

				276.64		1.437064

				276.66		1.437064

				276.68		1.437064

				276.7		1.437064

				276.72		1.437064

				276.74		1.437064

				276.76		1.437064

				276.78		1.437064

				276.8		1.437064

				276.82		1.437064

				276.85		1.437064

				276.87		1.437064

				276.89		1.437064

				276.91		1.437064

				276.93		1.437064

				276.95		1.437064

				276.97		1.437064

				276.99		1.437064

				277.01		1.437064

				277.03		1.437064

				277.06		1.437064

				277.08		1.437064

				277.1		1.437064

				277.12		1.437064

				277.14		1.437064

				277.16		1.437064

				277.18		1.437064

				277.2		1.437064

				277.22		1.437064

				277.24		1.437064

				277.26		1.437064

				277.29		1.437064

				277.31		1.437064

				277.33		1.437064

				277.35		1.437064

				277.37		1.437064

				277.39		1.437064

				277.41		1.437064

				277.43		1.437064

				277.45		1.437064

				277.47		1.437064

				277.5		1.442835

				277.52		1.437064

				277.54		1.437064

				277.56		1.442835

				277.58		1.437064

				277.6		1.442835

				277.62		1.437064

				277.64		1.442835

				277.66		1.437064

				277.68		1.442835

				277.71		1.437064

				277.73		1.442835

				277.75		1.437064

				277.77		1.442835

				277.79		1.437064

				277.81		1.437064

				277.83		1.437064

				277.85		1.437064

				277.87		1.437064

				277.89		1.437064

				277.92		1.437064

				277.94		1.437064

				277.96		1.437064

				277.98		1.437064

				278		1.437064

				278.02		1.437064

				278.04		1.437064

				278.06		1.437064

				278.08		1.437064

				278.1		1.437064

				278.12		1.437064

				278.15		1.437064

				278.17		1.431292

				278.19		1.431292

				278.21		1.431292

				278.23		1.431292

				278.25		1.431292

				278.27		1.431292

				278.29		1.431292

				278.31		1.431292

				278.33		1.431292

				278.36		1.431292

				278.38		1.431292

				278.4		1.431292

				278.42		1.431292

				278.44		1.431292

				278.46		1.431292

				278.48		1.431292

				278.5		1.431292

				278.52		1.431292

				278.54		1.431292

				278.57		1.431292

				278.59		1.431292

				278.61		1.431292

				278.63		1.431292

				278.65		1.431292

				278.67		1.431292

				278.69		1.431292

				278.71		1.431292

				278.73		1.431292

				278.75		1.431292

				278.78		1.431292

				278.8		1.431292

				278.82		1.431292

				278.84		1.431292

				278.86		1.431292

				278.88		1.431292

				278.9		1.431292

				278.92		1.431292

				278.94		1.425521

				278.96		1.431292

				278.99		1.425521

				279.01		1.425521

				279.03		1.425521

				279.05		1.425521

				279.07		1.425521

				279.09		1.425521

				279.11		1.425521

				279.13		1.425521

				279.15		1.425521

				279.17		1.425521

				279.2		1.425521

				279.22		1.425521

				279.24		1.425521

				279.26		1.425521

				279.28		1.425521

				279.3		1.425521

				279.32		1.425521

				279.34		1.425521

				279.36		1.425521

				279.38		1.425521

				279.4		1.425521

				279.43		1.425521

				279.45		1.425521

				279.47		1.41975

				279.49		1.41975

				279.51		1.41975

				279.53		1.41975

				279.55		1.41975

				279.57		1.41975

				279.59		1.41975

				279.62		1.41975

				279.64		1.41975

				279.66		1.41975

				279.68		1.41975

				279.7		1.41975

				279.72		1.41975

				279.74		1.41975

				279.76		1.41975

				279.78		1.41975

				279.8		1.41975

				279.83		1.41975

				279.85		1.41975

				279.87		1.41975

				279.89		1.41975

				279.91		1.41975

				279.93		1.41975

				279.95		1.41975

				279.97		1.41975

				279.99		1.41975

				280.01		1.41975

				280.04		1.41975

				280.06		1.41975

				280.08		1.41975

				280.1		1.41975

				280.12		1.41975

				280.14		1.41975

				280.16		1.41975

				280.18		1.41975

				280.2		1.41975

				280.22		1.41975

				280.25		1.41975

				280.27		1.41975

				280.29		1.41975

				280.31		1.41975

				280.33		1.41975

				280.35		1.41975

				280.37		1.41975

				280.39		1.41975

				280.41		1.41975

				280.43		1.41975

				280.46		1.41975

				280.48		1.41975

				280.5		1.41975

				280.52		1.41975

				280.54		1.41975

				280.56		1.41975

				280.58		1.41975

				280.6		1.41975

				280.62		1.41975

				280.65		1.41975

				280.67		1.41975

				280.69		1.41975

				280.71		1.41975

				280.73		1.41975

				280.75		1.41975

				280.77		1.41975

				280.79		1.41975

				280.81		1.41975

				280.83		1.41975

				280.86		1.41975

				280.88		1.41975

				280.9		1.41975

				280.92		1.41975

				280.94		1.41975

				280.96		1.41975

				280.98		1.41975

				281		1.41975

				281.02		1.41975

				281.04		1.41975

				281.07		1.41975

				281.09		1.41975

				281.11		1.41975

				281.13		1.41975

				281.15		1.41975

				281.17		1.41975

				281.19		1.41975

				281.21		1.41975

				281.23		1.41975

				281.25		1.41975

				281.28		1.41975

				281.3		1.41975

				281.32		1.41975

				281.34		1.41975

				281.36		1.41975

				281.38		1.41975

				281.4		1.41975

				281.42		1.41975

				281.44		1.41975

				281.46		1.41975

				281.49		1.41975

				281.51		1.41975

				281.53		1.41975

				281.55		1.41975

				281.57		1.41975

				281.59		1.41975

				281.61		1.41975

				281.63		1.41975

				281.65		1.41975

				281.67		1.41975

				281.7		1.41975

				281.72		1.41975

				281.74		1.41975

				281.76		1.41975

				281.78		1.41975

				281.8		1.41975

				281.82		1.41975

				281.84		1.413978

				281.86		1.413978

				281.88		1.413978

				281.91		1.413978

				281.93		1.413978

				281.95		1.413978

				281.97		1.413978

				281.99		1.413978

				282.01		1.413978

				282.03		1.413978

				282.05		1.413978

				282.07		1.413978

				282.09		1.413978

				282.12		1.413978

				282.14		1.413978

				282.16		1.413978

				282.18		1.413978

				282.2		1.413978

				282.22		1.413978

				282.24		1.413978

				282.26		1.413978

				282.28		1.413978

				282.3		1.413978

				282.33		1.413978

				282.35		1.413978

				282.37		1.413978

				282.39		1.413978

				282.41		1.413978

				282.43		1.413978

				282.45		1.413978

				282.47		1.413978

				282.49		1.413978

				282.51		1.413978

				282.54		1.413978

				282.56		1.413978

				282.58		1.413978

				282.6		1.413978

				282.62		1.413978

				282.64		1.413978

				282.66		1.408207

				282.68		1.408207

				282.7		1.413978

				282.72		1.408207

				282.75		1.413978

				282.77		1.408207

				282.79		1.408207

				282.81		1.408207

				282.83		1.408207

				282.85		1.408207

				282.87		1.408207

				282.89		1.408207

				282.91		1.408207

				282.93		1.408207

				282.96		1.408207

				282.98		1.408207

				283		1.408207

				283.02		1.408207

				283.04		1.408207

				283.06		1.408207

				283.08		1.408207

				283.1		1.408207

				283.12		1.408207

				283.15		1.408207

				283.17		1.408207

				283.19		1.408207

				283.21		1.408207

				283.23		1.408207

				283.25		1.408207

				283.27		1.408207

				283.29		1.408207

				283.31		1.408207

				283.33		1.408207

				283.36		1.408207

				283.38		1.408207

				283.4		1.408207

				283.42		1.408207

				283.44		1.408207

				283.46		1.408207

				283.48		1.408207

				283.5		1.408207

				283.52		1.408207

				283.55		1.408207

				283.57		1.408207

				283.59		1.408207

				283.61		1.408207

				283.63		1.408207

				283.65		1.408207

				283.67		1.408207

				283.69		1.408207

				283.71		1.408207

				283.73		1.408207

				283.76		1.408207

				283.78		1.408207

				283.8		1.408207

				283.82		1.408207

				283.84		1.408207

				283.86		1.408207

				283.88		1.408207

				283.9		1.413978

				283.92		1.408207

				283.94		1.408207

				283.97		1.413978

				283.99		1.408207

				284.01		1.408207

				284.03		1.413978

				284.05		1.413978

				284.07		1.413978

				284.09		1.413978

				284.11		1.408207

				284.13		1.413978

				284.16		1.408207

				284.18		1.413978

				284.2		1.413978

				284.22		1.413978

				284.24		1.408207

				284.26		1.408207

				284.28		1.408207

				284.3		1.408207

				284.32		1.408207

				284.34		1.408207

				284.37		1.408207

				284.39		1.408207

				284.41		1.408207

				284.43		1.408207

				284.45		1.408207

				284.47		1.408207

				284.49		1.408207

				284.51		1.408207

				284.53		1.408207

				284.56		1.408207

				284.58		1.408207

				284.6		1.408207

				284.62		1.408207

				284.64		1.408207

				284.66		1.408207

				284.68		1.408207

				284.7		1.408207

				284.72		1.402436

				284.74		1.402436

				284.77		1.402436

				284.79		1.402436

				284.81		1.402436

				284.83		1.402436

				284.85		1.402436

				284.87		1.402436

				284.89		1.402436

				284.91		1.402436

				284.93		1.402436

				284.96		1.402436

				284.98		1.402436

				285		1.402436

				285.02		1.402436

				285.04		1.402436

				285.06		1.402436

				285.08		1.402436

				285.1		1.402436

				285.12		1.402436

				285.14		1.402436

				285.17		1.402436

				285.19		1.402436

				285.21		1.402436

				285.23		1.402436

				285.25		1.402436

				285.27		1.402436

				285.29		1.402436

				285.31		1.402436

				285.33		1.402436

				285.35		1.402436

				285.38		1.402436

				285.4		1.402436

				285.42		1.396664

				285.44		1.396664

				285.46		1.396664

				285.48		1.396664

				285.5		1.402436

				285.52		1.396664

				285.54		1.402436

				285.57		1.396664

				285.59		1.402436

				285.61		1.396664

				285.63		1.402436

				285.65		1.402436

				285.67		1.402436

				285.69		1.396664

				285.71		1.396664

				285.73		1.396664

				285.75		1.396664

				285.78		1.396664

				285.8		1.396664

				285.82		1.396664

				285.84		1.396664

				285.86		1.396664

				285.88		1.396664

				285.9		1.396664

				285.92		1.396664

				285.94		1.396664

				285.97		1.396664

				285.99		1.396664

				286.01		1.402436

				286.03		1.396664

				286.05		1.396664

				286.07		1.402436

				286.09		1.396664

				286.11		1.396664

				286.13		1.396664

				286.15		1.396664

				286.18		1.396664

				286.2		1.396664

				286.22		1.396664

				286.24		1.396664

				286.26		1.396664

				286.28		1.396664

				286.3		1.396664

				286.32		1.396664

				286.34		1.396664

				286.36		1.396664

				286.39		1.396664

				286.41		1.396664

				286.43		1.396664

				286.45		1.396664

				286.47		1.396664

				286.49		1.396664

				286.51		1.396664

				286.53		1.396664

				286.55		1.396664

				286.58		1.396664

				286.6		1.396664

				286.62		1.396664

				286.64		1.396664

				286.66		1.390893

				286.68		1.396664

				286.7		1.390893

				286.72		1.396664

				286.74		1.390893

				286.76		1.396664

				286.79		1.396664

				286.81		1.396664

				286.83		1.390893

				286.85		1.396664

				286.87		1.396664

				286.89		1.396664

				286.91		1.396664

				286.93		1.396664

				286.95		1.390893

				286.98		1.396664

				287		1.396664

				287.02		1.396664

				287.04		1.396664

				287.06		1.396664

				287.08		1.396664

				287.1		1.396664

				287.12		1.396664

				287.14		1.396664

				287.16		1.390893

				287.19		1.390893

				287.21		1.390893

				287.23		1.390893

				287.25		1.390893

				287.27		1.390893

				287.29		1.390893

				287.31		1.390893

				287.33		1.390893

				287.35		1.390893

				287.38		1.390893

				287.4		1.390893

				287.42		1.390893

				287.44		1.396664

				287.46		1.390893

				287.48		1.390893

				287.5		1.390893

				287.52		1.390893

				287.54		1.390893

				287.56		1.390893

				287.59		1.390893

				287.61		1.390893

				287.63		1.390893

				287.65		1.390893

				287.67		1.390893

				287.69		1.390893

				287.71		1.390893

				287.73		1.390893

				287.75		1.390893

				287.78		1.390893

				287.8		1.390893

				287.82		1.390893

				287.84		1.390893

				287.86		1.390893

				287.88		1.390893

				287.9		1.390893

				287.92		1.390893

				287.94		1.390893

				287.96		1.390893

				287.99		1.385121

				288.01		1.390893

				288.03		1.390893

				288.05		1.385121

				288.07		1.390893

				288.09		1.385121

				288.11		1.385121

				288.13		1.385121

				288.15		1.385121

				288.18		1.385121

				288.2		1.385121

				288.22		1.385121

				288.24		1.385121

				288.26		1.385121

				288.28		1.385121

				288.3		1.385121

				288.32		1.385121

				288.34		1.385121

				288.37		1.385121

				288.39		1.385121

				288.41		1.385121

				288.43		1.385121

				288.45		1.385121

				288.47		1.385121

				288.49		1.385121

				288.51		1.385121

				288.53		1.385121

				288.55		1.385121

				288.58		1.385121

				288.6		1.385121

				288.62		1.385121

				288.64		1.385121

				288.66		1.385121

				288.68		1.385121

				288.7		1.385121

				288.72		1.385121

				288.74		1.385121

				288.77		1.385121

				288.79		1.385121

				288.81		1.385121

				288.83		1.385121

				288.85		1.385121

				288.87		1.385121

				288.89		1.385121

				288.91		1.385121

				288.93		1.385121

				288.95		1.385121

				288.98		1.385121

				289		1.385121

				289.02		1.385121

				289.04		1.385121

				289.06		1.385121

				289.08		1.385121

				289.1		1.385121

				289.12		1.385121

				289.14		1.385121

				289.16		1.385121

				289.19		1.385121

				289.21		1.385121

				289.23		1.385121

				289.25		1.385121

				289.27		1.385121

				289.29		1.385121

				289.31		1.385121

				289.33		1.385121

				289.35		1.385121

				289.38		1.385121

				289.4		1.385121

				289.42		1.385121

				289.44		1.385121

				289.46		1.385121

				289.48		1.37935

				289.5		1.385121

				289.52		1.37935

				289.54		1.37935

				289.56		1.37935

				289.59		1.37935

				289.61		1.37935

				289.63		1.37935

				289.65		1.37935

				289.67		1.37935

				289.69		1.37935

				289.71		1.37935

				289.73		1.37935

				289.75		1.37935

				289.78		1.37935

				289.8		1.37935

				289.82		1.37935

				289.84		1.37935

				289.86		1.385121

				289.88		1.37935

				289.9		1.37935

				289.92		1.37935

				289.94		1.37935

				289.97		1.37935

				289.99		1.37935

				290.01		1.37935

				290.03		1.37935

				290.05		1.37935

				290.07		1.37935

				290.09		1.37935

				290.11		1.37935

				290.13		1.37935

				290.15		1.37935

				290.18		1.37935

				290.2		1.37935

				290.22		1.37935

				290.24		1.37935

				290.26		1.37935

				290.28		1.37935

				290.3		1.37935

				290.32		1.373579

				290.34		1.37935

				290.37		1.37935

				290.39		1.373579

				290.41		1.373579

				290.43		1.373579

				290.45		1.373579

				290.47		1.373579

				290.49		1.373579

				290.51		1.373579

				290.53		1.367807

				290.55		1.373579

				290.58		1.373579

				290.6		1.373579

				290.62		1.373579

				290.64		1.373579

				290.66		1.373579

				290.68		1.373579

				290.7		1.373579

				290.72		1.373579

				290.74		1.373579

				290.77		1.373579

				290.79		1.373579

				290.81		1.373579

				290.83		1.373579

				290.85		1.367807

				290.87		1.367807

				290.89		1.367807

				290.91		1.367807

				290.93		1.367807

				290.95		1.367807

				290.98		1.367807

				291		1.367807

				291.02		1.367807

				291.04		1.367807

				291.06		1.367807

				291.08		1.367807

				291.1		1.367807

				291.12		1.367807

				291.14		1.367807

				291.17		1.367807

				291.19		1.367807

				291.21		1.367807

				291.23		1.367807

				291.25		1.367807

				291.27		1.367807

				291.29		1.373579

				291.31		1.367807

				291.33		1.367807

				291.36		1.367807

				291.38		1.367807

				291.4		1.367807

				291.42		1.367807

				291.44		1.367807

				291.46		1.367807

				291.48		1.367807

				291.5		1.367807

				291.52		1.367807

				291.55		1.367807

				291.57		1.367807

				291.59		1.367807

				291.61		1.367807

				291.63		1.367807

				291.65		1.367807

				291.67		1.367807

				291.69		1.367807

				291.71		1.367807

				291.73		1.367807

				291.76		1.367807

				291.78		1.367807

				291.8		1.367807

				291.82		1.367807

				291.84		1.367807

				291.86		1.367807

				291.88		1.367807

				291.9		1.367807

				291.92		1.367807

				291.95		1.367807

				291.97		1.367807

				291.99		1.367807

				292.01		1.367807

				292.03		1.362036

				292.05		1.362036

				292.07		1.362036

				292.09		1.362036

				292.11		1.367807

				292.14		1.367807

				292.16		1.367807

				292.18		1.367807

				292.2		1.367807

				292.22		1.367807

				292.24		1.367807

				292.26		1.367807

				292.28		1.367807

				292.3		1.362036

				292.32		1.362036

				292.35		1.362036

				292.37		1.362036

				292.39		1.367807

				292.41		1.362036

				292.43		1.367807

				292.45		1.362036

				292.47		1.362036

				292.49		1.367807

				292.51		1.362036

				292.54		1.367807

				292.56		1.367807

				292.58		1.367807

				292.6		1.362036

				292.62		1.367807

				292.64		1.367807

				292.66		1.362036

				292.68		1.367807

				292.7		1.362036

				292.72		1.367807

				292.75		1.362036

				292.77		1.367807

				292.79		1.362036

				292.81		1.362036

				292.83		1.362036

				292.85		1.362036

				292.87		1.362036

				292.89		1.362036

				292.91		1.362036

				292.93		1.362036

				292.96		1.362036

				292.98		1.362036

				293		1.362036

				293.02		1.362036

				293.04		1.362036

				293.06		1.362036

				293.08		1.362036

				293.1		1.362036

				293.12		1.362036

				293.15		1.362036

				293.17		1.362036

				293.19		1.362036

				293.21		1.362036

				293.23		1.362036

				293.25		1.362036

				293.27		1.362036

				293.29		1.362036

				293.31		1.362036

				293.33		1.362036

				293.36		1.362036

				293.38		1.362036

				293.4		1.362036

				293.42		1.362036

				293.44		1.356265

				293.46		1.356265

				293.48		1.362036

				293.5		1.362036

				293.52		1.356265

				293.54		1.356265

				293.57		1.356265

				293.59		1.356265

				293.61		1.356265

				293.63		1.356265

				293.65		1.356265

				293.67		1.356265

				293.69		1.356265

				293.71		1.356265

				293.73		1.356265

				293.75		1.356265

				293.78		1.356265

				293.8		1.356265

				293.82		1.356265

				293.84		1.356265

				293.86		1.356265

				293.88		1.356265

				293.9		1.356265

				293.92		1.356265

				293.94		1.356265

				293.97		1.356265

				293.99		1.356265

				294.01		1.356265

				294.03		1.356265

				294.05		1.356265

				294.07		1.356265

				294.09		1.356265

				294.11		1.356265

				294.13		1.356265

				294.15		1.356265

				294.18		1.356265

				294.2		1.356265

				294.22		1.356265

				294.24		1.356265

				294.26		1.356265

				294.28		1.356265

				294.3		1.356265

				294.32		1.356265

				294.34		1.356265

				294.37		1.356265

				294.39		1.356265

				294.41		1.356265

				294.43		1.356265

				294.45		1.356265

				294.47		1.356265

				294.49		1.356265

				294.51		1.356265

				294.53		1.356265

				294.55		1.356265

				294.58		1.356265

				294.6		1.356265

				294.62		1.356265

				294.64		1.356265

				294.66		1.356265

				294.68		1.356265

				294.7		1.356265

				294.72		1.356265

				294.74		1.356265

				294.77		1.356265

				294.79		1.356265

				294.81		1.356265

				294.83		1.356265

				294.85		1.356265

				294.87		1.356265

				294.89		1.356265

				294.91		1.356265

				294.93		1.356265

				294.96		1.356265

				294.98		1.356265

				295		1.356265

				295.02		1.356265

				295.04		1.356265

				295.06		1.356265

				295.08		1.356265

				295.1		1.356265

				295.12		1.356265

				295.14		1.356265

				295.17		1.362036

				295.19		1.356265

				295.21		1.356265

				295.23		1.356265

				295.25		1.356265

				295.27		1.356265

				295.29		1.356265

				295.31		1.356265

				295.33		1.356265

				295.36		1.350493

				295.38		1.350493

				295.4		1.350493

				295.42		1.350493

				295.44		1.350493

				295.46		1.350493

				295.48		1.350493

				295.5		1.350493

				295.52		1.350493

				295.54		1.350493

				295.57		1.350493

				295.59		1.350493

				295.61		1.350493

				295.63		1.350493

				295.65		1.350493

				295.67		1.350493

				295.69		1.350493

				295.71		1.350493

				295.73		1.350493

				295.76		1.350493

				295.78		1.350493

				295.8		1.350493

				295.82		1.350493

				295.84		1.350493

				295.86		1.350493

				295.88		1.350493

				295.9		1.350493

				295.92		1.350493

				295.95		1.350493

				295.97		1.350493

				295.99		1.350493

				296.01		1.350493

				296.03		1.350493

				296.05		1.350493

				296.07		1.350493

				296.09		1.350493

				296.11		1.350493

				296.13		1.350493

				296.16		1.350493

				296.18		1.350493

				296.2		1.350493

				296.22		1.350493

				296.24		1.350493

				296.26		1.350493

				296.28		1.350493

				296.3		1.350493

				296.32		1.350493

				296.35		1.350493

				296.37		1.350493

				296.39		1.350493

				296.41		1.350493

				296.43		1.350493

				296.45		1.350493

				296.47		1.350493

				296.49		1.350493

				296.51		1.350493

				296.54		1.350493

				296.56		1.344722

				296.58		1.350493

				296.6		1.350493

				296.62		1.350493

				296.64		1.350493

				296.66		1.350493

				296.68		1.344722

				296.7		1.350493

				296.72		1.344722

				296.75		1.350493

				296.77		1.344722

				296.79		1.344722

				296.81		1.344722

				296.83		1.344722

				296.85		1.344722

				296.87		1.344722

				296.89		1.344722

				296.91		1.344722

				296.94		1.344722

				296.96		1.344722

				296.98		1.344722

				297		1.344722

				297.02		1.344722

				297.04		1.344722

				297.06		1.344722

				297.08		1.344722

				297.1		1.344722

				297.12		1.344722

				297.15		1.350493

				297.17		1.344722

				297.19		1.350493

				297.21		1.350493

				297.23		1.350493

				297.25		1.350493

				297.27		1.350493

				297.29		1.350493

				297.31		1.350493

				297.34		1.350493

				297.36		1.350493

				297.38		1.350493

				297.4		1.350493

				297.42		1.350493

				297.44		1.356265

				297.46		1.356265

				297.48		1.350493

				297.5		1.356265

				297.52		1.356265

				297.55		1.356265

				297.57		1.356265

				297.59		1.356265

				297.61		1.356265

				297.63		1.356265

				297.65		1.356265

				297.67		1.356265

				297.69		1.356265

				297.71		1.356265

				297.74		1.356265

				297.76		1.356265

				297.78		1.356265

				297.8		1.356265

				297.82		1.356265

				297.84		1.356265

				297.86		1.356265

				297.88		1.356265

				297.9		1.356265

				297.92		1.356265

				297.95		1.356265

				297.97		1.356265

				297.99		1.356265

				298.01		1.356265

				298.03		1.356265

				298.05		1.356265

				298.07		1.356265

				298.09		1.356265

				298.11		1.356265

				298.14		1.356265

				298.16		1.356265

				298.18		1.356265

				298.2		1.356265

				298.22		1.350493

				298.24		1.350493

				298.26		1.350493

				298.28		1.350493

				298.3		1.350493

				298.33		1.350493

				298.35		1.350493

				298.37		1.350493

				298.39		1.350493

				298.41		1.350493

				298.43		1.350493

				298.45		1.350493

				298.47		1.350493

				298.49		1.350493

				298.52		1.350493

				298.54		1.350493

				298.56		1.350493

				298.58		1.350493

				298.6		1.350493

				298.62		1.350493

				298.64		1.350493

				298.66		1.350493

				298.68		1.350493

				298.71		1.350493

				298.73		1.350493

				298.75		1.350493

				298.77		1.350493

				298.79		1.350493

				298.81		1.356265

				298.83		1.350493

				298.85		1.350493

				298.87		1.350493

				298.9		1.350493

				298.92		1.350493

				298.94		1.350493

				298.96		1.350493

				298.98		1.350493

				299		1.350493

				299.02		1.350493

				299.04		1.350493

				299.06		1.350493

				299.09		1.350493

				299.11		1.350493

				299.13		1.350493

				299.15		1.350493

				299.17		1.350493

				299.19		1.350493

				299.21		1.350493

				299.23		1.350493

				299.25		1.350493

				299.28		1.350493

				299.3		1.350493

				299.32		1.350493

				299.34		1.350493

				299.36		1.350493

				299.38		1.344722

				299.4		1.344722

				299.42		1.344722

				299.44		1.344722

				299.47		1.344722

				299.49		1.344722

				299.51		1.344722

				299.53		1.344722

				299.55		1.344722

				299.57		1.344722

				299.59		1.344722

				299.61		1.344722

				299.63		1.344722

				299.66		1.344722

				299.68		1.344722

				299.7		1.344722

				299.72		1.344722

				299.74		1.344722

				299.76		1.344722

				299.78		1.338951

				299.8		1.344722

				299.82		1.344722

				299.85		1.344722

				299.87		1.344722

				299.89		1.344722

				299.91		1.344722

				299.93		1.338951

				299.95		1.338951

				299.97		1.338951

				299.99		1.338951

				300.01		1.338951

				300.04		1.338951

				300.06		1.338951

				300.08		1.338951

				300.1		1.338951

				300.12		1.338951

				300.14		1.333179

				300.16		1.338951

				300.18		1.338951

				300.2		1.338951

				300.23		1.333179

				300.25		1.333179

				300.27		1.333179

				300.29		1.333179

				300.31		1.333179

				300.33		1.333179

				300.35		1.333179

				300.37		1.333179

				300.39		1.333179

				300.42		1.333179

				300.44		1.333179

				300.46		1.333179

				300.48		1.333179

				300.5		1.333179

				300.52		1.333179

				300.54		1.327408

				300.56		1.327408

				300.58		1.327408

				300.61		1.327408

				300.63		1.327408

				300.65		1.327408

				300.67		1.327408

				300.69		1.327408

				300.71		1.327408

				300.73		1.321637

				300.75		1.321637

				300.77		1.321637

				300.8		1.321637

				300.82		1.321637

				300.84		1.321637

				300.86		1.321637

				300.88		1.321637

				300.9		1.321637

				300.92		1.321637

				300.94		1.321637

				300.96		1.321637

				300.98		1.321637

				301.01		1.321637

				301.03		1.321637

				301.05		1.321637

				301.07		1.321637

				301.09		1.321637

				301.11		1.321637

				301.13		1.321637

				301.15		1.315865

				301.17		1.321637

				301.2		1.315865

				301.22		1.315865

				301.24		1.315865

				301.26		1.315865

				301.28		1.315865

				301.3		1.315865

				301.32		1.315865

				301.34		1.315865

				301.36		1.315865

				301.39		1.315865

				301.41		1.315865

				301.43		1.310094

				301.45		1.310094

				301.47		1.310094

				301.49		1.310094

				301.51		1.310094

				301.53		1.310094

				301.55		1.310094

				301.58		1.310094

				301.6		1.310094

				301.62		1.310094

				301.64		1.310094

				301.66		1.310094

				301.68		1.304323

				301.7		1.310094

				301.72		1.310094

				301.74		1.310094

				301.77		1.310094

				301.79		1.310094

				301.81		1.310094

				301.83		1.304323

				301.85		1.304323

				301.87		1.304323

				301.89		1.304323

				301.91		1.304323

				301.93		1.304323

				301.95		1.304323

				301.98		1.304323

				302		1.304323

				302.02		1.304323

				302.04		1.304323

				302.06		1.304323

				302.08		1.304323

				302.1		1.298551

				302.12		1.304323

				302.14		1.304323

				302.17		1.304323

				302.19		1.304323

				302.21		1.304323

				302.23		1.304323

				302.25		1.298551

				302.27		1.298551

				302.29		1.298551

				302.31		1.304323

				302.33		1.298551

				302.36		1.298551

				302.38		1.304323

				302.4		1.298551

				302.42		1.298551

				302.44		1.298551

				302.46		1.298551

				302.48		1.298551

				302.5		1.298551

				302.52		1.298551

				302.55		1.298551

				302.57		1.304323

				302.59		1.298551

				302.61		1.298551

				302.63		1.304323

				302.65		1.298551

				302.67		1.298551

				302.69		1.298551

				302.71		1.304323

				302.74		1.298551

				302.76		1.298551

				302.78		1.298551

				302.8		1.298551

				302.82		1.298551

				302.84		1.298551

				302.86		1.298551

				302.88		1.298551

				302.9		1.298551

				302.93		1.298551

				302.95		1.298551

				302.97		1.298551

				302.99		1.298551

				303.01		1.298551

				303.03		1.298551

				303.05		1.298551

				303.07		1.298551

				303.1		1.298551

				303.12		1.29278

				303.14		1.298551

				303.16		1.298551

				303.18		1.298551

				303.2		1.29278

				303.22		1.29278

				303.24		1.29278

				303.26		1.29278

				303.29		1.298551

				303.31		1.29278

				303.33		1.29278

				303.35		1.29278

				303.37		1.29278

				303.39		1.29278

				303.41		1.29278

				303.43		1.29278

				303.45		1.29278

				303.48		1.29278

				303.5		1.29278

				303.52		1.29278

				303.54		1.29278

				303.56		1.29278

				303.58		1.29278

				303.6		1.29278

				303.62		1.29278

				303.64		1.29278

				303.67		1.29278

				303.69		1.29278

				303.71		1.29278

				303.73		1.29278

				303.75		1.29278

				303.77		1.29278

				303.79		1.287009

				303.81		1.29278

				303.83		1.287009

				303.86		1.287009

				303.88		1.287009

				303.9		1.287009

				303.92		1.287009

				303.94		1.287009

				303.96		1.287009

				303.98		1.287009

				304		1.287009

				304.02		1.287009

				304.05		1.287009

				304.07		1.287009

				304.09		1.287009

				304.11		1.287009

				304.13		1.287009

				304.15		1.287009

				304.17		1.287009

				304.19		1.287009

				304.21		1.287009

				304.24		1.287009

				304.26		1.287009

				304.28		1.287009

				304.3		1.287009

				304.32		1.287009

				304.34		1.287009

				304.36		1.287009

				304.38		1.287009

				304.4		1.287009

				304.43		1.287009

				304.45		1.287009

				304.47		1.287009

				304.49		1.287009

				304.51		1.287009

				304.53		1.287009

				304.55		1.287009

				304.57		1.287009

				304.59		1.281237

				304.62		1.287009

				304.64		1.281237

				304.66		1.281237

				304.68		1.281237

				304.7		1.281237

				304.72		1.281237

				304.74		1.281237

				304.76		1.281237

				304.78		1.281237

				304.81		1.281237

				304.83		1.281237

				304.85		1.281237

				304.87		1.281237

				304.89		1.281237

				304.91		1.281237

				304.93		1.281237

				304.95		1.281237

				304.97		1.275466

				305		1.275466

				305.02		1.275466

				305.04		1.275466

				305.06		1.275466

				305.08		1.275466

				305.1		1.275466

				305.12		1.275466

				305.14		1.275466

				305.16		1.275466

				305.18		1.275466

				305.21		1.275466

				305.23		1.275466

				305.25		1.275466

				305.27		1.275466

				305.29		1.275466

				305.31		1.275466

				305.33		1.275466

				305.35		1.275466

				305.37		1.275466

				305.4		1.275466

				305.42		1.275466

				305.44		1.275466

				305.46		1.275466

				305.48		1.269695

				305.5		1.269695

				305.52		1.269695

				305.54		1.269695

				305.56		1.269695

				305.59		1.269695

				305.61		1.269695

				305.63		1.275466

				305.65		1.275466

				305.67		1.275466

				305.69		1.275466

				305.71		1.275466

				305.73		1.275466

				305.75		1.275466

				305.78		1.275466

				305.8		1.275466

				305.82		1.275466

				305.84		1.275466

				305.86		1.275466

				305.88		1.275466

				305.9		1.275466

				305.92		1.275466

				305.94		1.275466

				305.97		1.275466

				305.99		1.275466

				306.01		1.275466

				306.03		1.275466

				306.05		1.275466

				306.07		1.275466

				306.09		1.275466

				306.11		1.275466

				306.13		1.275466

				306.16		1.275466

				306.18		1.275466

				306.2		1.275466

				306.22		1.275466

				306.24		1.275466

				306.26		1.275466

				306.28		1.275466

				306.3		1.275466

				306.32		1.275466

				306.35		1.275466

				306.37		1.275466

				306.39		1.275466

				306.41		1.275466

				306.43		1.275466

				306.45		1.275466

				306.47		1.269695

				306.49		1.269695

				306.51		1.269695

				306.54		1.269695

				306.56		1.275466

				306.58		1.275466

				306.6		1.275466

				306.62		1.275466

				306.64		1.275466

				306.66		1.275466

				306.68		1.275466

				306.7		1.275466

				306.73		1.275466

				306.75		1.275466

				306.77		1.275466

				306.79		1.275466

				306.81		1.275466

				306.83		1.275466

				306.85		1.275466

				306.87		1.275466

				306.9		1.275466

				306.92		1.275466

				306.94		1.275466

				306.96		1.275466

				306.98		1.275466

				307		1.275466

				307.02		1.275466

				307.04		1.275466

				307.06		1.275466

				307.09		1.281237

				307.11		1.281237

				307.13		1.281237

				307.15		1.281237

				307.17		1.281237

				307.19		1.281237

				307.21		1.281237

				307.23		1.281237

				307.25		1.281237

				307.28		1.281237

				307.3		1.281237

				307.32		1.281237

				307.34		1.281237

				307.36		1.281237

				307.38		1.281237

				307.4		1.281237

				307.42		1.281237

				307.44		1.281237

				307.47		1.281237

				307.49		1.281237

				307.51		1.281237

				307.53		1.281237

				307.55		1.281237

				307.57		1.281237

				307.59		1.281237

				307.61		1.287009

				307.64		1.281237

				307.66		1.287009

				307.68		1.287009

				307.7		1.287009

				307.72		1.287009

				307.74		1.281237

				307.76		1.287009

				307.78		1.287009

				307.8		1.281237

				307.83		1.281237

				307.85		1.287009

				307.87		1.287009

				307.89		1.287009

				307.91		1.281237

				307.93		1.281237

				307.95		1.281237

				307.97		1.281237

				307.99		1.281237

				308.02		1.287009

				308.04		1.281237

				308.06		1.281237

				308.08		1.281237

				308.1		1.287009

				308.12		1.287009

				308.14		1.287009

				308.16		1.287009

				308.18		1.287009

				308.21		1.287009

				308.23		1.287009

				308.25		1.287009

				308.27		1.281237

				308.29		1.287009

				308.31		1.287009

				308.33		1.287009

				308.35		1.287009

				308.38		1.287009

				308.4		1.287009

				308.42		1.287009

				308.44		1.287009

				308.46		1.287009

				308.48		1.287009

				308.5		1.287009

				308.52		1.287009

				308.54		1.287009

				308.57		1.287009

				308.59		1.287009

				308.61		1.287009

				308.63		1.287009

				308.65		1.287009

				308.67		1.287009

				308.69		1.287009

				308.71		1.287009

				308.73		1.287009

				308.76		1.287009

				308.78		1.287009

				308.8		1.287009

				308.82		1.287009

				308.84		1.287009

				308.86		1.287009

				308.88		1.287009

				308.9		1.287009

				308.92		1.287009

				308.95		1.287009

				308.97		1.287009

				308.99		1.29278

				309.01		1.287009

				309.03		1.29278

				309.05		1.287009

				309.07		1.287009

				309.09		1.287009

				309.11		1.287009

				309.14		1.287009

				309.16		1.287009

				309.18		1.287009

				309.2		1.287009

				309.22		1.287009

				309.24		1.287009

				309.26		1.287009

				309.28		1.287009

				309.3		1.287009

				309.33		1.287009

				309.35		1.287009

				309.37		1.287009

				309.39		1.287009

				309.41		1.287009

				309.43		1.287009

				309.45		1.287009

				309.47		1.287009

				309.49		1.287009

				309.52		1.287009

				309.54		1.287009

				309.56		1.287009

				309.58		1.287009

				309.6		1.287009

				309.62		1.287009

				309.64		1.287009

				309.66		1.287009

				309.68		1.287009

				309.71		1.287009

				309.73		1.287009

				309.75		1.287009

				309.77		1.281237

				309.79		1.281237

				309.81		1.281237

				309.83		1.281237

				309.85		1.281237

				309.88		1.281237

				309.9		1.281237

				309.92		1.281237

				309.94		1.281237

				309.96		1.281237

				309.98		1.281237

				310		1.281237

				310.02		1.281237

				310.04		1.281237

				310.07		1.281237

				310.09		1.281237

				310.11		1.281237

				310.13		1.281237

				310.15		1.281237

				310.17		1.281237

				310.19		1.281237

				310.21		1.281237

				310.23		1.281237

				310.26		1.281237

				310.28		1.281237

				310.3		1.281237

				310.32		1.281237

				310.34		1.281237

				310.36		1.281237

				310.38		1.275466

				310.4		1.275466

				310.42		1.275466

				310.45		1.275466

				310.47		1.275466

				310.49		1.275466

				310.51		1.275466

				310.53		1.275466

				310.55		1.275466

				310.57		1.275466

				310.59		1.275466

				310.62		1.275466

				310.64		1.275466

				310.66		1.275466

				310.68		1.275466

				310.7		1.275466

				310.72		1.275466

				310.74		1.275466

				310.76		1.275466

				310.78		1.275466

				310.81		1.275466

				310.83		1.275466

				310.85		1.275466

				310.87		1.275466

				310.89		1.275466

				310.91		1.275466

				310.93		1.275466

				310.95		1.275466

				310.98		1.275466

				311		1.275466

				311.02		1.275466

				311.04		1.275466

				311.06		1.275466

				311.08		1.275466

				311.1		1.275466

				311.12		1.275466

				311.14		1.275466

				311.17		1.275466

				311.19		1.275466

				311.21		1.269695

				311.23		1.275466

				311.25		1.275466

				311.27		1.275466

				311.29		1.269695

				311.31		1.275466

				311.34		1.269695

				311.36		1.269695

				311.38		1.269695

				311.4		1.269695

				311.42		1.269695

				311.44		1.269695

				311.46		1.275466

				311.48		1.269695

				311.5		1.269695

				311.53		1.275466

				311.55		1.269695

				311.57		1.269695

				311.59		1.269695

				311.61		1.275466

				311.63		1.269695

				311.65		1.269695

				311.67		1.269695

				311.7		1.269695

				311.72		1.275466

				311.74		1.275466

				311.76		1.275466

				311.78		1.275466

				311.8		1.275466

				311.82		1.275466

				311.84		1.275466

				311.87		1.275466

				311.89		1.275466

				311.91		1.275466

				311.93		1.275466

				311.95		1.275466

				311.97		1.275466

				311.99		1.275466

				312.01		1.275466

				312.03		1.275466

				312.06		1.275466

				312.08		1.275466

				312.1		1.275466

				312.12		1.275466

				312.14		1.275466

				312.16		1.275466

				312.18		1.275466

				312.2		1.275466

				312.22		1.275466

				312.25		1.275466

				312.27		1.275466

				312.29		1.275466

				312.31		1.275466

				312.33		1.275466

				312.35		1.275466

				312.37		1.275466

				312.39		1.275466

				312.42		1.275466

				312.44		1.275466

				312.46		1.275466

				312.48		1.275466

				312.5		1.275466

				312.52		1.275466

				312.54		1.275466

				312.56		1.275466

				312.58		1.275466

				312.61		1.275466

				312.63		1.275466

				312.65		1.275466

				312.67		1.275466

				312.69		1.275466

				312.71		1.275466

				312.73		1.275466

				312.75		1.275466

				312.77		1.275466

				312.8		1.275466

				312.82		1.275466

				312.84		1.275466

				312.86		1.275466

				312.88		1.275466

				312.9		1.275466

				312.92		1.281237

				312.94		1.275466

				312.97		1.275466

				312.99		1.275466

				313.01		1.275466

				313.03		1.275466

				313.05		1.275466

				313.07		1.275466

				313.09		1.275466

				313.11		1.275466

				313.13		1.275466

				313.16		1.275466

				313.18		1.275466

				313.2		1.275466

				313.22		1.275466

				313.24		1.275466

				313.26		1.275466

				313.28		1.275466

				313.3		1.275466

				313.33		1.275466

				313.35		1.275466

				313.37		1.275466

				313.39		1.275466

				313.41		1.275466

				313.43		1.281237

				313.45		1.281237

				313.47		1.281237

				313.49		1.281237

				313.52		1.275466

				313.54		1.281237

				313.56		1.275466

				313.58		1.281237

				313.6		1.275466

				313.62		1.275466

				313.64		1.275466

				313.66		1.275466

				313.68		1.275466

				313.71		1.275466

				313.73		1.275466

				313.75		1.275466

				313.77		1.275466

				313.79		1.275466

				313.81		1.275466

				313.83		1.269695

				313.85		1.275466

				313.88		1.269695

				313.9		1.275466

				313.92		1.269695

				313.94		1.269695

				313.96		1.269695

				313.98		1.269695

				314		1.269695

				314.02		1.269695

				314.04		1.269695

				314.07		1.269695

				314.09		1.269695

				314.11		1.269695

				314.13		1.269695

				314.15		1.269695

				314.17		1.269695

				314.19		1.269695

				314.21		1.269695

				314.24		1.269695

				314.26		1.269695

				314.28		1.269695

				314.3		1.269695

				314.32		1.269695

				314.34		1.269695

				314.36		1.269695

				314.38		1.269695

				314.4		1.269695

				314.43		1.269695

				314.45		1.269695

				314.47		1.269695

				314.49		1.269695

				314.51		1.269695

				314.53		1.269695

				314.55		1.269695

				314.57		1.269695

				314.6		1.269695

				314.62		1.269695

				314.64		1.269695

				314.66		1.269695

				314.68		1.269695

				314.7		1.269695

				314.72		1.269695

				314.74		1.269695

				314.76		1.269695

				314.79		1.269695

				314.81		1.269695

				314.83		1.269695

				314.85		1.269695

				314.87		1.269695

				314.89		1.269695

				314.91		1.269695

				314.93		1.269695

				314.95		1.269695

				314.98		1.269695

				315		1.269695

				315.02		1.269695

				315.04		1.269695

				315.06		1.269695

				315.08		1.269695

				315.1		1.269695

				315.12		1.269695

				315.15		1.269695

				315.17		1.269695

				315.19		1.263923

				315.21		1.263923

				315.23		1.269695

				315.25		1.263923

				315.27		1.263923

				315.29		1.263923

				315.31		1.263923

				315.34		1.263923

				315.36		1.263923

				315.38		1.263923

				315.4		1.263923

				315.42		1.263923

				315.44		1.263923

				315.46		1.263923

				315.48		1.263923

				315.51		1.263923

				315.53		1.263923

				315.55		1.263923

				315.57		1.258152

				315.59		1.258152

				315.61		1.258152

				315.63		1.258152

				315.65		1.258152

				315.67		1.258152

				315.7		1.258152

				315.72		1.258152

				315.74		1.258152

				315.76		1.258152

				315.78		1.258152

				315.8		1.258152

				315.82		1.258152

				315.84		1.258152

				315.87		1.263923

				315.89		1.263923

				315.91		1.258152

				315.93		1.263923

				315.95		1.263923

				315.97		1.258152

				315.99		1.258152

				316.01		1.258152

				316.04		1.263923

				316.06		1.263923

				316.08		1.263923

				316.1		1.258152

				316.12		1.258152

				316.14		1.258152

				316.16		1.258152

				316.18		1.258152

				316.2		1.258152

				316.23		1.258152

				316.25		1.258152

				316.27		1.258152

				316.29		1.258152

				316.31		1.258152

				316.33		1.258152

				316.35		1.258152

				316.37		1.258152

				316.4		1.258152

				316.42		1.258152

				316.44		1.258152

				316.46		1.258152

				316.48		1.258152

				316.5		1.258152

				316.52		1.258152

				316.54		1.258152

				316.56		1.258152

				316.59		1.258152

				316.61		1.258152

				316.63		1.258152

				316.65		1.258152

				316.67		1.258152

				316.69		1.258152

				316.71		1.258152

				316.73		1.258152

				316.76		1.258152

				316.78		1.258152

				316.8		1.258152

				316.82		1.258152

				316.84		1.258152

				316.86		1.258152

				316.88		1.258152

				316.9		1.258152

				316.92		1.258152

				316.95		1.258152

				316.97		1.258152

				316.99		1.258152

				317.01		1.258152

				317.03		1.258152

				317.05		1.258152

				317.07		1.258152

				317.09		1.258152

				317.12		1.252381

				317.14		1.252381

				317.16		1.252381

				317.18		1.252381

				317.2		1.252381

				317.22		1.252381

				317.24		1.252381

				317.26		1.252381

				317.28		1.252381

				317.31		1.252381

				317.33		1.252381

				317.35		1.252381

				317.37		1.252381

				317.39		1.252381

				317.41		1.252381

				317.43		1.252381

				317.45		1.258152

				317.48		1.252381

				317.5		1.258152

				317.52		1.258152

				317.54		1.258152

				317.56		1.258152

				317.58		1.258152

				317.6		1.258152

				317.62		1.258152

				317.64		1.258152

				317.67		1.258152

				317.69		1.258152

				317.71		1.258152

				317.73		1.258152

				317.75		1.258152

				317.77		1.258152

				317.79		1.258152

				317.81		1.258152

				317.84		1.258152

				317.86		1.258152

				317.88		1.258152

				317.9		1.258152

				317.92		1.258152

				317.94		1.258152

				317.96		1.258152

				317.98		1.258152

				318		1.258152

				318.03		1.258152

				318.05		1.258152

				318.07		1.258152

				318.09		1.258152

				318.11		1.258152

				318.13		1.258152

				318.15		1.258152

				318.17		1.258152

				318.2		1.258152

				318.22		1.258152

				318.24		1.258152

				318.26		1.258152

				318.28		1.258152

				318.3		1.258152

				318.32		1.258152

				318.34		1.258152

				318.36		1.258152

				318.39		1.258152

				318.41		1.258152

				318.43		1.263923

				318.45		1.263923

				318.47		1.258152

				318.49		1.258152

				318.51		1.258152

				318.53		1.258152

				318.56		1.258152

				318.58		1.258152

				318.6		1.258152

				318.62		1.258152

				318.64		1.258152

				318.66		1.258152

				318.68		1.258152

				318.7		1.258152

				318.72		1.258152

				318.75		1.258152

				318.77		1.258152

				318.79		1.258152

				318.81		1.258152

				318.83		1.258152

				318.85		1.258152

				318.87		1.258152

				318.89		1.258152

				318.92		1.258152

				318.94		1.258152

				318.96		1.258152

				318.98		1.258152

				319		1.258152

				319.02		1.258152

				319.04		1.258152

				319.06		1.258152

				319.09		1.258152

				319.11		1.258152

				319.13		1.258152

				319.15		1.258152

				319.17		1.258152

				319.19		1.258152

				319.21		1.258152

				319.23		1.263923

				319.25		1.258152

				319.28		1.263923

				319.3		1.263923

				319.32		1.258152

				319.34		1.258152

				319.36		1.263923

				319.38		1.263923

				319.4		1.263923

				319.42		1.263923

				319.45		1.263923

				319.47		1.263923

				319.49		1.263923

				319.51		1.258152

				319.53		1.258152

				319.55		1.258152

				319.57		1.258152

				319.59		1.258152

				319.61		1.258152

				319.64		1.258152

				319.66		1.258152

				319.68		1.258152

				319.7		1.258152

				319.72		1.258152

				319.74		1.258152

				319.76		1.258152

				319.78		1.258152

				319.81		1.258152

				319.83		1.258152

				319.85		1.258152

				319.87		1.258152

				319.89		1.263923

				319.91		1.258152

				319.93		1.263923

				319.95		1.258152

				319.98		1.258152

				320		1.258152

				320.02		1.258152

				320.04		1.258152

				320.06		1.258152

				320.08		1.258152

				320.1		1.258152

				320.12		1.258152

				320.14		1.258152

				320.17		1.258152

				320.19		1.258152

				320.21		1.258152

				320.23		1.258152

				320.25		1.258152

				320.27		1.258152

				320.29		1.258152

				320.31		1.263923

				320.34		1.263923

				320.36		1.258152

				320.38		1.263923

				320.4		1.263923

				320.42		1.258152

				320.44		1.258152

				320.46		1.258152

				320.48		1.258152

				320.5		1.258152

				320.53		1.258152

				320.55		1.258152

				320.57		1.258152

				320.59		1.258152

				320.61		1.258152

				320.63		1.258152

				320.65		1.258152

				320.67		1.258152

				320.7		1.258152

				320.72		1.258152

				320.74		1.258152

				320.76		1.258152

				320.78		1.258152

				320.8		1.258152

				320.82		1.258152

				320.84		1.258152

				320.86		1.258152

				320.89		1.258152

				320.91		1.258152

				320.93		1.258152

				320.95		1.258152

				320.97		1.258152

				320.99		1.258152

				321.01		1.258152

				321.03		1.258152

				321.05		1.258152

				321.08		1.258152

				321.1		1.258152

				321.12		1.258152

				321.14		1.258152

				321.16		1.258152

				321.18		1.258152

				321.2		1.258152

				321.22		1.258152

				321.25		1.258152

				321.27		1.258152

				321.29		1.258152

				321.31		1.258152

				321.33		1.258152

				321.35		1.258152

				321.37		1.258152

				321.39		1.258152

				321.41		1.258152

				321.44		1.258152

				321.46		1.258152

				321.48		1.258152

				321.5		1.258152

				321.52		1.258152

				321.54		1.258152

				321.56		1.258152

				321.58		1.258152

				321.6		1.258152

				321.63		1.258152

				321.65		1.258152

				321.67		1.258152

				321.69		1.258152

				321.71		1.258152

				321.73		1.258152

				321.75		1.252381

				321.77		1.258152

				321.79		1.252381

				321.82		1.252381

				321.84		1.252381

				321.86		1.252381

				321.88		1.252381

				321.9		1.252381

				321.92		1.252381

				321.94		1.252381

				321.96		1.246609

				321.98		1.246609

				322.01		1.246609

				322.03		1.246609

				322.05		1.246609

				322.07		1.246609

				322.09		1.246609

				322.11		1.246609

				322.13		1.246609

				322.15		1.246609

				322.17		1.246609

				322.2		1.246609

				322.22		1.246609

				322.24		1.246609

				322.26		1.246609

				322.28		1.246609

				322.3		1.246609

				322.32		1.246609

				322.34		1.246609

				322.36		1.246609

				322.39		1.246609

				322.41		1.246609

				322.43		1.240838

				322.45		1.240838

				322.47		1.240838

				322.49		1.240838

				322.51		1.240838

				322.53		1.240838

				322.56		1.240838

				322.58		1.240838

				322.6		1.240838

				322.62		1.240838

				322.64		1.240838

				322.66		1.240838

				322.68		1.240838

				322.7		1.240838

				322.72		1.240838

				322.75		1.240838

				322.77		1.240838

				322.79		1.240838

				322.81		1.240838

				322.83		1.240838

				322.85		1.240838

				322.87		1.240838

				322.89		1.240838

				322.91		1.240838

				322.94		1.240838

				322.96		1.240838

				322.98		1.240838

				323		1.235067

				323.02		1.235067

				323.04		1.235067

				323.06		1.235067

				323.08		1.235067

				323.1		1.235067

				323.13		1.235067

				323.15		1.235067

				323.17		1.235067

				323.19		1.235067

				323.21		1.235067

				323.23		1.235067

				323.25		1.235067

				323.27		1.235067

				323.29		1.235067

				323.32		1.235067

				323.34		1.235067

				323.36		1.235067

				323.38		1.235067

				323.4		1.235067

				323.42		1.235067

				323.44		1.235067

				323.46		1.229295

				323.48		1.235067

				323.51		1.235067

				323.53		1.229295

				323.55		1.229295

				323.57		1.229295

				323.59		1.229295

				323.61		1.229295

				323.63		1.229295

				323.65		1.229295

				323.67		1.229295

				323.7		1.229295

				323.72		1.229295

				323.74		1.229295

				323.76		1.229295

				323.78		1.229295

				323.8		1.229295

				323.82		1.229295

				323.84		1.229295

				323.87		1.229295

				323.89		1.229295

				323.91		1.229295

				323.93		1.229295

				323.95		1.229295

				323.97		1.229295

				323.99		1.229295

				324.01		1.229295

				324.03		1.229295

				324.06		1.229295

				324.08		1.229295

				324.1		1.229295

				324.12		1.229295

				324.14		1.229295

				324.16		1.229295

				324.18		1.229295

				324.2		1.229295

				324.22		1.229295

				324.25		1.229295

				324.27		1.229295

				324.29		1.229295

				324.31		1.229295

				324.33		1.229295

				324.35		1.229295

				324.37		1.229295

				324.39		1.229295

				324.41		1.229295

				324.44		1.229295

				324.46		1.229295

				324.48		1.229295

				324.5		1.229295

				324.52		1.229295

				324.54		1.229295

				324.56		1.229295

				324.58		1.229295

				324.6		1.229295

				324.63		1.229295

				324.65		1.229295

				324.67		1.229295

				324.69		1.229295

				324.71		1.229295

				324.73		1.229295

				324.75		1.229295

				324.77		1.229295

				324.79		1.229295

				324.82		1.229295

				324.84		1.229295

				324.86		1.229295

				324.88		1.223524

				324.9		1.223524

				324.92		1.223524

				324.94		1.223524

				324.96		1.223524

				324.99		1.223524

				325.01		1.223524

				325.03		1.223524

				325.05		1.223524

				325.07		1.223524

				325.09		1.223524

				325.11		1.223524

				325.13		1.223524

				325.15		1.223524

				325.18		1.223524

				325.2		1.223524

				325.22		1.229295

				325.24		1.223524

				325.26		1.223524

				325.28		1.223524

				325.3		1.223524

				325.32		1.223524

				325.34		1.223524

				325.37		1.223524

				325.39		1.223524

				325.41		1.223524

				325.43		1.223524

				325.45		1.223524

				325.47		1.223524

				325.49		1.223524

				325.51		1.223524

				325.53		1.223524

				325.56		1.223524

				325.58		1.223524

				325.6		1.223524

				325.62		1.223524

				325.64		1.223524

				325.66		1.223524

				325.68		1.223524

				325.7		1.223524

				325.72		1.223524

				325.75		1.223524

				325.77		1.223524

				325.79		1.223524

				325.81		1.223524

				325.83		1.223524

				325.85		1.223524

				325.87		1.223524

				325.89		1.217753

				325.91		1.217753

				325.94		1.217753

				325.96		1.217753

				325.98		1.217753

				326		1.217753

				326.02		1.217753

				326.04		1.217753

				326.06		1.217753

				326.08		1.217753

				326.1		1.217753

				326.13		1.217753

				326.15		1.217753

				326.17		1.217753

				326.19		1.217753

				326.21		1.217753

				326.23		1.217753

				326.25		1.217753

				326.27		1.217753

				326.3		1.217753

				326.32		1.217753

				326.34		1.217753

				326.36		1.217753

				326.38		1.217753

				326.4		1.217753

				326.42		1.217753

				326.44		1.217753

				326.46		1.217753

				326.49		1.217753

				326.51		1.217753

				326.53		1.217753

				326.55		1.217753

				326.57		1.217753

				326.59		1.217753

				326.61		1.217753

				326.63		1.217753

				326.65		1.217753

				326.68		1.217753

				326.7		1.217753

				326.72		1.217753

				326.74		1.217753

				326.76		1.217753

				326.78		1.217753

				326.8		1.217753

				326.82		1.217753

				326.84		1.217753

				326.87		1.217753

				326.89		1.217753

				326.91		1.217753

				326.93		1.217753

				326.95		1.217753

				326.97		1.217753

				326.99		1.217753

				327.01		1.217753

				327.03		1.217753

				327.06		1.217753

				327.08		1.217753

				327.1		1.217753

				327.12		1.217753

				327.14		1.217753

				327.16		1.217753

				327.18		1.217753

				327.2		1.217753

				327.22		1.217753

				327.25		1.217753

				327.27		1.217753

				327.29		1.217753

				327.31		1.217753

				327.33		1.217753

				327.35		1.217753

				327.37		1.217753

				327.39		1.217753

				327.42		1.217753

				327.44		1.217753

				327.46		1.217753

				327.48		1.217753

				327.5		1.217753

				327.52		1.217753

				327.54		1.217753

				327.56		1.217753

				327.58		1.217753

				327.61		1.217753

				327.63		1.217753

				327.65		1.217753

				327.67		1.217753

				327.69		1.217753

				327.71		1.217753

				327.73		1.217753

				327.75		1.217753

				327.77		1.217753

				327.8		1.217753

				327.82		1.217753

				327.84		1.217753

				327.86		1.217753

				327.88		1.217753

				327.9		1.217753

				327.92		1.217753

				327.94		1.223524

				327.97		1.217753

				327.99		1.223524

				328.01		1.223524

				328.03		1.223524

				328.05		1.223524

				328.07		1.223524

				328.09		1.223524

				328.11		1.223524

				328.13		1.223524

				328.16		1.223524

				328.18		1.223524

				328.2		1.223524

				328.22		1.223524

				328.24		1.223524

				328.26		1.223524

				328.28		1.223524

				328.3		1.223524

				328.32		1.223524

				328.35		1.223524

				328.37		1.223524

				328.39		1.223524

				328.41		1.229295

				328.43		1.229295

				328.45		1.229295

				328.47		1.229295

				328.49		1.229295

				328.51		1.229295

				328.54		1.223524

				328.56		1.229295

				328.58		1.229295

				328.6		1.229295

				328.62		1.223524

				328.64		1.229295

				328.66		1.223524

				328.68		1.229295

				328.7		1.229295

				328.73		1.229295

				328.75		1.223524

				328.77		1.229295

				328.79		1.229295

				328.81		1.229295

				328.83		1.229295

				328.85		1.229295

				328.87		1.229295

				328.9		1.229295

				328.92		1.229295

				328.94		1.229295

				328.96		1.229295

				328.98		1.229295

				329		1.229295

				329.02		1.229295

				329.04		1.229295

				329.06		1.229295

				329.09		1.229295

				329.11		1.229295

				329.13		1.229295

				329.15		1.229295

				329.17		1.229295

				329.19		1.229295

				329.21		1.229295

				329.23		1.229295

				329.25		1.229295

				329.28		1.229295

				329.3		1.229295

				329.32		1.229295

				329.34		1.229295

				329.36		1.229295

				329.38		1.229295

				329.4		1.229295

				329.42		1.229295

				329.44		1.229295

				329.47		1.229295

				329.49		1.229295

				329.51		1.229295

				329.53		1.229295

				329.55		1.229295

				329.57		1.229295

				329.59		1.229295

				329.61		1.229295

				329.63		1.229295

				329.66		1.229295

				329.68		1.229295

				329.7		1.229295

				329.72		1.229295

				329.74		1.229295

				329.76		1.229295

				329.78		1.229295

				329.8		1.229295

				329.82		1.229295

				329.85		1.229295

				329.87		1.229295

				329.89		1.229295

				329.91		1.229295

				329.93		1.229295

				329.95		1.229295

				329.97		1.229295

				329.99		1.229295

				330.02		1.229295

				330.04		1.229295

				330.06		1.229295

				330.08		1.229295

				330.1		1.229295

				330.12		1.229295

				330.14		1.229295

				330.16		1.223524

				330.18		1.229295

				330.21		1.229295

				330.23		1.223524

				330.25		1.223524

				330.27		1.223524

				330.29		1.229295

				330.31		1.223524

				330.33		1.229295

				330.35		1.229295

				330.37		1.229295

				330.4		1.229295

				330.42		1.229295

				330.44		1.229295

				330.46		1.229295

				330.48		1.229295

				330.5		1.229295

				330.52		1.229295

				330.54		1.229295

				330.56		1.229295

				330.59		1.229295

				330.61		1.229295

				330.63		1.229295

				330.65		1.229295

				330.67		1.223524

				330.69		1.223524

				330.71		1.223524

				330.73		1.223524

				330.75		1.223524

				330.78		1.223524

				330.8		1.223524

				330.82		1.223524

				330.84		1.223524

				330.86		1.229295

				330.88		1.223524

				330.9		1.229295

				330.92		1.223524

				330.94		1.229295

				330.97		1.229295

				330.99		1.223524

				331.01		1.223524

				331.03		1.223524

				331.05		1.223524

				331.07		1.229295

				331.09		1.223524

				331.11		1.223524

				331.13		1.223524

				331.15		1.223524

				331.18		1.223524

				331.2		1.223524

				331.22		1.223524

				331.24		1.223524

				331.26		1.223524

				331.28		1.223524

				331.3		1.217753

				331.32		1.223524

				331.35		1.217753

				331.37		1.223524

				331.39		1.217753

				331.41		1.217753

				331.43		1.223524

				331.45		1.223524

				331.47		1.217753

				331.49		1.217753

				331.51		1.217753

				331.54		1.217753

				331.56		1.217753

				331.58		1.217753

				331.6		1.217753

				331.62		1.217753

				331.64		1.217753

				331.66		1.217753

				331.68		1.217753

				331.7		1.217753

				331.73		1.217753

				331.75		1.217753

				331.77		1.217753

				331.79		1.217753

				331.81		1.217753

				331.83		1.217753

				331.85		1.217753

				331.87		1.217753

				331.89		1.217753

				331.92		1.217753

				331.94		1.217753

				331.96		1.217753

				331.98		1.217753

				332		1.217753

				332.02		1.217753

				332.04		1.217753

				332.06		1.217753

				332.08		1.217753

				332.11		1.217753

				332.13		1.217753

				332.15		1.217753

				332.17		1.217753

				332.19		1.217753

				332.21		1.211981

				332.23		1.217753

				332.25		1.217753

				332.27		1.217753

				332.3		1.217753

				332.32		1.217753

				332.34		1.217753

				332.36		1.211981

				332.38		1.211981

				332.4		1.211981

				332.42		1.211981

				332.44		1.211981

				332.46		1.211981

				332.49		1.211981

				332.51		1.211981

				332.53		1.211981

				332.55		1.211981

				332.57		1.211981

				332.59		1.211981

				332.61		1.211981

				332.63		1.211981

				332.66		1.211981

				332.68		1.211981

				332.7		1.211981

				332.72		1.211981

				332.74		1.20621

				332.76		1.20621

				332.78		1.211981

				332.8		1.211981

				332.82		1.20621

				332.85		1.20621

				332.87		1.20621

				332.89		1.20621

				332.91		1.20621

				332.93		1.20621

				332.95		1.20621

				332.97		1.20621

				332.99		1.20621

				333.01		1.20621

				333.04		1.20621

				333.06		1.20621

				333.08		1.20621

				333.1		1.20621

				333.12		1.20621

				333.14		1.20621

				333.16		1.20621

				333.18		1.20621

				333.2		1.20621

				333.23		1.20621

				333.25		1.20621

				333.27		1.20621

				333.29		1.20621

				333.31		1.20621

				333.33		1.20621

				333.35		1.211981

				333.37		1.211981

				333.39		1.211981

				333.42		1.211981

				333.44		1.211981

				333.46		1.211981

				333.48		1.211981

				333.5		1.211981

				333.52		1.211981

				333.54		1.20621

				333.56		1.20621

				333.58		1.20621

				333.61		1.20621

				333.63		1.20621

				333.65		1.20621

				333.67		1.20621

				333.69		1.20621

				333.71		1.20621

				333.73		1.20621

				333.75		1.20621

				333.77		1.20621

				333.8		1.20621

				333.82		1.20621

				333.84		1.20621

				333.86		1.211981

				333.88		1.20621

				333.9		1.20621

				333.92		1.20621

				333.94		1.20621

				333.96		1.20621

				333.99		1.20621

				334.01		1.20621

				334.03		1.20621

				334.05		1.20621

				334.07		1.20621

				334.09		1.20621

				334.11		1.20621

				334.13		1.20621

				334.15		1.20621

				334.18		1.20621

				334.2		1.20621

				334.22		1.20621

				334.24		1.20621

				334.26		1.20621

				334.28		1.20621

				334.3		1.211981

				334.32		1.20621

				334.34		1.20621

				334.37		1.211981

				334.39		1.20621

				334.41		1.211981

				334.43		1.211981

				334.45		1.211981

				334.47		1.211981

				334.49		1.211981

				334.51		1.211981

				334.53		1.211981

				334.55		1.211981

				334.58		1.211981

				334.6		1.211981

				334.62		1.211981

				334.64		1.211981

				334.66		1.211981

				334.68		1.211981

				334.7		1.211981

				334.72		1.211981

				334.74		1.211981

				334.77		1.211981

				334.79		1.211981

				334.81		1.211981

				334.83		1.211981

				334.85		1.211981

				334.87		1.217753

				334.89		1.211981

				334.91		1.211981

				334.93		1.211981

				334.96		1.217753

				334.98		1.217753

				335		1.217753

				335.02		1.217753

				335.04		1.211981

				335.06		1.217753

				335.08		1.211981

				335.1		1.211981

				335.12		1.211981

				335.15		1.211981

				335.17		1.211981

				335.19		1.211981

				335.21		1.217753

				335.23		1.211981

				335.25		1.211981

				335.27		1.211981

				335.29		1.211981

				335.31		1.211981

				335.34		1.211981

				335.36		1.217753

				335.38		1.211981

				335.4		1.211981

				335.42		1.211981

				335.44		1.211981

				335.46		1.211981

				335.48		1.211981

				335.5		1.211981

				335.53		1.211981

				335.55		1.211981

				335.57		1.211981

				335.59		1.211981

				335.61		1.211981

				335.63		1.211981

				335.65		1.211981

				335.67		1.211981

				335.69		1.211981

				335.72		1.211981

				335.74		1.211981

				335.76		1.211981

				335.78		1.211981

				335.8		1.211981

				335.82		1.211981

				335.84		1.211981

				335.86		1.211981

				335.88		1.211981

				335.91		1.211981

				335.93		1.211981

				335.95		1.211981

				335.97		1.211981

				335.99		1.20621

				336.01		1.211981

				336.03		1.20621

				336.05		1.20621

				336.07		1.20621

				336.1		1.20621

				336.12		1.20621

				336.14		1.20621

				336.16		1.20621

				336.18		1.20621

				336.2		1.20621

				336.22		1.20621

				336.24		1.20621

				336.26		1.20621

				336.29		1.20621

				336.31		1.20621

				336.33		1.20621

				336.35		1.20621

				336.37		1.20621

				336.39		1.20621

				336.41		1.20621

				336.43		1.20621

				336.45		1.200439

				336.48		1.200439

				336.5		1.200439

				336.52		1.200439

				336.54		1.200439

				336.56		1.200439

				336.58		1.200439

				336.6		1.200439

				336.62		1.200439

				336.64		1.200439

				336.67		1.200439

				336.69		1.200439

				336.71		1.200439

				336.73		1.200439

				336.75		1.194667

				336.77		1.194667

				336.79		1.194667

				336.81		1.194667

				336.83		1.194667

				336.86		1.194667

				336.88		1.194667

				336.9		1.194667

				336.92		1.194667

				336.94		1.194667

				336.96		1.194667

				336.98		1.194667

				337		1.194667

				337.02		1.194667

				337.05		1.194667

				337.07		1.194667

				337.09		1.194667

				337.11		1.188896

				337.13		1.188896

				337.15		1.188896

				337.17		1.188896

				337.19		1.188896

				337.21		1.188896

				337.24		1.188896

				337.26		1.188896

				337.28		1.188896

				337.3		1.188896

				337.32		1.183125

				337.34		1.188896

				337.36		1.188896

				337.38		1.183125

				337.4		1.183125

				337.43		1.183125

				337.45		1.183125

				337.47		1.183125

				337.49		1.183125

				337.51		1.183125

				337.53		1.183125

				337.55		1.183125

				337.57		1.183125

				337.59		1.183125

				337.62		1.183125

				337.64		1.183125

				337.66		1.183125

				337.68		1.183125

				337.7		1.183125

				337.72		1.183125

				337.74		1.183125

				337.76		1.183125

				337.79		1.188896

				337.81		1.188896

				337.83		1.183125

				337.85		1.188896

				337.87		1.188896

				337.89		1.183125

				337.91		1.183125

				337.93		1.188896

				337.95		1.188896

				337.98		1.183125

				338		1.183125

				338.02		1.183125

				338.04		1.183125

				338.06		1.183125

				338.08		1.183125

				338.1		1.183125

				338.12		1.183125

				338.14		1.183125

				338.17		1.188896

				338.19		1.183125

				338.21		1.188896

				338.23		1.188896

				338.25		1.188896

				338.27		1.188896

				338.29		1.183125

				338.31		1.183125

				338.33		1.183125

				338.36		1.188896

				338.38		1.188896

				338.4		1.188896

				338.42		1.188896

				338.44		1.188896

				338.46		1.183125

				338.48		1.183125

				338.5		1.183125

				338.52		1.183125

				338.55		1.183125

				338.57		1.183125

				338.59		1.183125

				338.61		1.183125

				338.63		1.183125

				338.65		1.183125

				338.67		1.188896

				338.69		1.183125

				338.71		1.188896

				338.74		1.188896

				338.76		1.188896

				338.78		1.188896

				338.8		1.188896

				338.82		1.188896

				338.84		1.188896

				338.86		1.188896

				338.88		1.188896

				338.9		1.188896

				338.93		1.188896

				338.95		1.183125

				338.97		1.188896

				338.99		1.183125

				339.01		1.183125

				339.03		1.183125

				339.05		1.183125

				339.07		1.183125

				339.09		1.183125

				339.12		1.183125

				339.14		1.183125

				339.16		1.183125

				339.18		1.183125

				339.2		1.183125

				339.22		1.183125

				339.24		1.183125

				339.26		1.183125

				339.28		1.183125

				339.31		1.183125

				339.33		1.188896

				339.35		1.188896

				339.37		1.183125

				339.39		1.188896

				339.41		1.188896

				339.43		1.183125

				339.45		1.183125

				339.47		1.183125

				339.5		1.183125

				339.52		1.183125

				339.54		1.183125

				339.56		1.183125

				339.58		1.183125

				339.6		1.183125

				339.62		1.183125

				339.64		1.183125

				339.66		1.183125

				339.69		1.183125

				339.71		1.183125

				339.73		1.183125

				339.75		1.183125

				339.77		1.183125

				339.79		1.183125

				339.81		1.183125

				339.83		1.183125

				339.85		1.183125

				339.88		1.183125

				339.9		1.183125

				339.92		1.183125

				339.94		1.183125

				339.96		1.183125

				339.98		1.183125

				340		1.183125

				340.02		1.177353

				340.04		1.183125

				340.07		1.177353

				340.09		1.183125

				340.11		1.177353

				340.13		1.183125

				340.15		1.177353

				340.17		1.177353

				340.19		1.177353

				340.21		1.177353

				340.23		1.177353

				340.25		1.177353

				340.28		1.177353

				340.3		1.177353

				340.32		1.177353

				340.34		1.177353

				340.36		1.177353

				340.38		1.177353

				340.4		1.177353

				340.42		1.177353

				340.44		1.177353

				340.47		1.177353

				340.49		1.177353

				340.51		1.177353

				340.53		1.177353

				340.55		1.177353

				340.57		1.177353

				340.59		1.177353

				340.61		1.177353

				340.63		1.177353

				340.66		1.177353

				340.68		1.177353

				340.7		1.177353

				340.72		1.177353

				340.74		1.177353

				340.76		1.177353

				340.78		1.171582

				340.8		1.171582

				340.82		1.171582

				340.85		1.171582

				340.87		1.171582

				340.89		1.171582

				340.91		1.171582

				340.93		1.171582

				340.95		1.171582

				340.97		1.171582

				340.99		1.171582

				341.01		1.171582

				341.04		1.171582

				341.06		1.171582

				341.08		1.171582

				341.1		1.171582

				341.12		1.171582

				341.14		1.171582

				341.16		1.171582

				341.18		1.171582

				341.2		1.171582

				341.23		1.171582

				341.25		1.171582

				341.27		1.171582

				341.29		1.171582

				341.31		1.171582

				341.33		1.171582

				341.35		1.171582

				341.37		1.171582

				341.39		1.171582

				341.42		1.171582

				341.44		1.171582

				341.46		1.171582

				341.48		1.171582

				341.5		1.171582

				341.52		1.171582

				341.54		1.171582

				341.56		1.171582

				341.58		1.171582

				341.61		1.171582

				341.63		1.171582

				341.65		1.171582

				341.67		1.171582

				341.69		1.171582

				341.71		1.165811

				341.73		1.165811

				341.75		1.165811

				341.77		1.165811

				341.8		1.165811

				341.82		1.165811

				341.84		1.165811

				341.86		1.165811

				341.88		1.165811

				341.9		1.165811

				341.92		1.165811

				341.94		1.165811

				341.96		1.165811

				341.99		1.165811

				342.01		1.165811

				342.03		1.165811

				342.05		1.165811

				342.07		1.165811

				342.09		1.165811

				342.11		1.165811

				342.13		1.165811

				342.15		1.165811

				342.18		1.160039

				342.2		1.165811

				342.22		1.165811

				342.24		1.165811

				342.26		1.160039

				342.28		1.165811

				342.3		1.165811

				342.32		1.165811

				342.34		1.165811

				342.37		1.165811

				342.39		1.165811

				342.41		1.160039

				342.43		1.160039

				342.45		1.160039

				342.47		1.160039

				342.49		1.165811

				342.51		1.165811

				342.53		1.165811

				342.56		1.165811

				342.58		1.165811

				342.6		1.165811

				342.62		1.165811

				342.64		1.160039

				342.66		1.165811

				342.68		1.160039

				342.7		1.160039

				342.72		1.160039

				342.75		1.160039

				342.77		1.160039

				342.79		1.160039

				342.81		1.165811

				342.83		1.160039

				342.85		1.160039

				342.87		1.165811

				342.89		1.165811

				342.91		1.160039

				342.94		1.160039

				342.96		1.165811

				342.98		1.160039

				343		1.165811

				343.02		1.165811

				343.04		1.165811

				343.06		1.165811

				343.08		1.165811

				343.1		1.165811

				343.13		1.165811

				343.15		1.165811

				343.17		1.165811

				343.19		1.165811

				343.21		1.165811

				343.23		1.165811

				343.25		1.165811

				343.27		1.165811

				343.29		1.165811

				343.32		1.165811

				343.34		1.165811

				343.36		1.165811

				343.38		1.165811

				343.4		1.165811

				343.42		1.165811

				343.44		1.165811

				343.46		1.165811

				343.48		1.165811

				343.51		1.165811

				343.53		1.165811

				343.55		1.165811

				343.57		1.165811

				343.59		1.165811

				343.61		1.165811

				343.63		1.165811

				343.65		1.165811

				343.67		1.165811

				343.69		1.165811

				343.72		1.165811

				343.74		1.165811

				343.76		1.165811

				343.78		1.165811

				343.8		1.171582

				343.82		1.171582

				343.84		1.171582

				343.86		1.171582

				343.88		1.171582

				343.91		1.171582

				343.93		1.171582

				343.95		1.171582

				343.97		1.171582

				343.99		1.171582

				344.01		1.171582

				344.03		1.171582

				344.05		1.171582

				344.07		1.171582

				344.1		1.171582

				344.12		1.171582

				344.14		1.171582

				344.16		1.171582

				344.18		1.171582

				344.2		1.171582

				344.22		1.171582

				344.24		1.171582

				344.26		1.171582

				344.29		1.171582

				344.31		1.171582

				344.33		1.171582

				344.35		1.171582

				344.37		1.171582

				344.39		1.171582

				344.41		1.171582

				344.43		1.171582

				344.45		1.171582

				344.48		1.171582

				344.5		1.171582

				344.52		1.171582

				344.54		1.171582

				344.56		1.171582

				344.58		1.171582

				344.6		1.171582

				344.62		1.171582

				344.64		1.171582

				344.67		1.171582

				344.69		1.171582

				344.71		1.171582

				344.73		1.171582

				344.75		1.171582

				344.77		1.171582

				344.79		1.171582

				344.81		1.171582

				344.83		1.171582

				344.85		1.171582

				344.88		1.171582

				344.9		1.171582

				344.92		1.171582

				344.94		1.171582

				344.96		1.171582

				344.98		1.171582

				345		1.171582

				345.02		1.171582

				345.04		1.171582

				345.07		1.171582

				345.09		1.171582

				345.11		1.171582

				345.13		1.171582

				345.15		1.171582

				345.17		1.171582

				345.19		1.171582

				345.21		1.171582

				345.23		1.171582

				345.26		1.171582

				345.28		1.171582

				345.3		1.171582

				345.32		1.171582

				345.34		1.171582

				345.36		1.171582

				345.38		1.171582

				345.4		1.171582

				345.42		1.171582

				345.45		1.171582

				345.47		1.171582

				345.49		1.171582

				345.51		1.171582

				345.53		1.171582

				345.55		1.171582

				345.57		1.171582

				345.59		1.171582

				345.61		1.171582

				345.64		1.171582

				345.66		1.171582

				345.68		1.171582

				345.7		1.171582

				345.72		1.171582

				345.74		1.171582

				345.76		1.171582

				345.78		1.171582

				345.8		1.171582

				345.83		1.171582

				345.85		1.171582

				345.87		1.171582

				345.89		1.171582

				345.91		1.171582

				345.93		1.171582

				345.95		1.171582

				345.97		1.171582

				345.99		1.171582

				346.02		1.171582

				346.04		1.171582

				346.06		1.171582

				346.08		1.171582

				346.1		1.171582

				346.12		1.171582

				346.14		1.171582

				346.16		1.171582

				346.18		1.171582

				346.2		1.171582

				346.23		1.171582

				346.25		1.171582

				346.27		1.171582

				346.29		1.171582

				346.31		1.171582

				346.33		1.171582

				346.35		1.171582

				346.37		1.171582

				346.39		1.171582

				346.42		1.171582

				346.44		1.177353

				346.46		1.177353

				346.48		1.177353

				346.5		1.177353

				346.52		1.177353

				346.54		1.177353

				346.56		1.177353

				346.58		1.177353

				346.61		1.177353

				346.63		1.177353

				346.65		1.177353

				346.67		1.177353

				346.69		1.177353

				346.71		1.177353

				346.73		1.177353

				346.75		1.177353

				346.77		1.177353

				346.8		1.177353

				346.82		1.177353

				346.84		1.177353

				346.86		1.177353

				346.88		1.177353

				346.9		1.177353

				346.92		1.177353

				346.94		1.177353

				346.96		1.177353

				346.99		1.177353

				347.01		1.177353

				347.03		1.183125

				347.05		1.183125

				347.07		1.183125

				347.09		1.183125

				347.11		1.183125

				347.13		1.183125

				347.15		1.183125

				347.18		1.177353

				347.2		1.177353

				347.22		1.183125

				347.24		1.177353

				347.26		1.177353

				347.28		1.177353

				347.3		1.177353

				347.32		1.177353

				347.34		1.177353

				347.37		1.177353

				347.39		1.177353

				347.41		1.177353

				347.43		1.177353

				347.45		1.183125

				347.47		1.183125

				347.49		1.183125

				347.51		1.183125

				347.53		1.183125

				347.56		1.183125

				347.58		1.183125

				347.6		1.183125

				347.62		1.183125

				347.64		1.183125

				347.66		1.183125

				347.68		1.183125

				347.7		1.183125

				347.72		1.183125

				347.75		1.183125

				347.77		1.183125

				347.79		1.183125

				347.81		1.183125

				347.83		1.183125

				347.85		1.183125

				347.87		1.183125

				347.89		1.183125

				347.91		1.183125

				347.94		1.183125

				347.96		1.183125

				347.98		1.183125

				348		1.183125

				348.02		1.183125

				348.04		1.188896

				348.06		1.183125

				348.08		1.183125

				348.1		1.183125

				348.12		1.183125

				348.15		1.183125

				348.17		1.183125

				348.19		1.183125

				348.21		1.183125

				348.23		1.183125

				348.25		1.183125

				348.27		1.183125

				348.29		1.183125

				348.31		1.183125

				348.34		1.183125

				348.36		1.183125

				348.38		1.183125

				348.4		1.183125

				348.42		1.183125

				348.44		1.183125

				348.46		1.183125

				348.48		1.183125

				348.5		1.183125

				348.53		1.183125

				348.55		1.183125

				348.57		1.183125

				348.59		1.183125

				348.61		1.183125

				348.63		1.183125

				348.65		1.183125

				348.67		1.183125

				348.69		1.183125

				348.72		1.183125

				348.74		1.183125

				348.76		1.183125

				348.78		1.183125

				348.8		1.183125

				348.82		1.183125

				348.84		1.183125

				348.86		1.183125

				348.88		1.183125

				348.91		1.183125

				348.93		1.183125

				348.95		1.183125

				348.97		1.183125

				348.99		1.183125

				349.01		1.183125

				349.03		1.183125

				349.05		1.183125

				349.07		1.183125

				349.1		1.183125

				349.12		1.177353

				349.14		1.177353

				349.16		1.177353

				349.18		1.177353

				349.2		1.177353

				349.22		1.177353

				349.24		1.177353

				349.27		1.177353

				349.29		1.177353

				349.31		1.177353

				349.33		1.183125

				349.35		1.177353

				349.37		1.183125

				349.39		1.183125

				349.41		1.183125

				349.44		1.183125

				349.46		1.183125

				349.48		1.183125

				349.5		1.183125

				349.52		1.183125

				349.54		1.183125

				349.56		1.177353

				349.58		1.177353

				349.61		1.183125

				349.63		1.177353

				349.65		1.177353

				349.67		1.177353

				349.69		1.177353

				349.71		1.177353

				349.73		1.177353

				349.76		1.177353

				349.78		1.177353

				349.8		1.177353

				349.82		1.177353

				349.84		1.177353

				349.86		1.177353

				349.88		1.177353

				349.9		1.177353

				349.93		1.177353

				349.95		1.177353

				349.97		1.177353

				349.99		1.177353

				350.01		1.177353

				350.03		1.177353

				350.05		1.177353

				350.08		1.177353

				350.1		1.171582

				350.12		1.177353

				350.14		1.171582

				350.16		1.171582

				350.18		1.177353

				350.2		1.171582

				350.22		1.177353

				350.25		1.171582

				350.27		1.171582

				350.29		1.171582

				350.31		1.171582

				350.33		1.171582

				350.35		1.171582

				350.37		1.171582

				350.39		1.171582

				350.41		1.171582

				350.44		1.171582

				350.46		1.171582

				350.48		1.171582

				350.5		1.171582

				350.52		1.171582

				350.54		1.171582

				350.56		1.171582

				350.58		1.171582

				350.61		1.171582

				350.63		1.171582

				350.65		1.171582

				350.67		1.171582

				350.69		1.171582

				350.71		1.171582

				350.73		1.171582

				350.75		1.171582

				350.77		1.171582

				350.8		1.171582

				350.82		1.171582

				350.84		1.171582

				350.86		1.171582

				350.88		1.171582

				350.9		1.171582

				350.92		1.171582

				350.94		1.171582

				350.97		1.171582

				350.99		1.171582

				351.01		1.171582

				351.03		1.171582

				351.05		1.171582

				351.07		1.171582

				351.09		1.165811

				351.11		1.171582

				351.13		1.171582

				351.16		1.171582

				351.18		1.171582

				351.2		1.171582

				351.22		1.171582

				351.24		1.171582

				351.26		1.171582

				351.28		1.171582

				351.3		1.171582

				351.32		1.171582

				351.35		1.171582

				351.37		1.171582

				351.39		1.171582

				351.41		1.171582

				351.43		1.171582

				351.45		1.171582

				351.47		1.171582

				351.49		1.171582

				351.52		1.171582

				351.54		1.171582

				351.56		1.171582

				351.58		1.171582

				351.6		1.171582

				351.62		1.171582

				351.64		1.171582

				351.66		1.171582

				351.68		1.171582

				351.71		1.171582

				351.73		1.171582

				351.75		1.171582

				351.77		1.171582

				351.79		1.171582

				351.81		1.171582

				351.83		1.171582

				351.85		1.171582

				351.88		1.171582

				351.9		1.171582

				351.92		1.171582

				351.94		1.171582

				351.96		1.171582

				351.98		1.171582

				352		1.171582

				352.02		1.171582

				352.04		1.171582

				352.07		1.171582

				352.09		1.171582

				352.11		1.171582

				352.13		1.171582

				352.15		1.171582

				352.17		1.171582

				352.19		1.171582

				352.21		1.171582

				352.24		1.171582

				352.26		1.171582

				352.28		1.171582

				352.3		1.171582

				352.32		1.171582

				352.34		1.171582

				352.36		1.171582

				352.38		1.171582

				352.41		1.171582

				352.43		1.171582

				352.45		1.171582

				352.47		1.171582

				352.49		1.171582

				352.51		1.171582

				352.53		1.171582

				352.55		1.171582

				352.57		1.171582

				352.6		1.171582

				352.62		1.171582

				352.64		1.171582

				352.66		1.171582

				352.68		1.171582

				352.7		1.171582

				352.72		1.177353

				352.74		1.177353

				352.77		1.177353

				352.79		1.177353

				352.81		1.177353

				352.83		1.177353

				352.85		1.177353

				352.87		1.177353

				352.89		1.177353

				352.91		1.177353

				352.94		1.177353

				352.96		1.177353

				352.98		1.177353

				353		1.177353

				353.02		1.177353

				353.04		1.177353

				353.06		1.177353

				353.08		1.177353

				353.1		1.177353

				353.13		1.177353

				353.15		1.177353

				353.17		1.177353

				353.19		1.177353

				353.21		1.177353

				353.23		1.177353

				353.25		1.177353

				353.27		1.177353

				353.3		1.177353

				353.32		1.177353

				353.34		1.177353

				353.36		1.177353

				353.38		1.177353

				353.4		1.177353

				353.42		1.177353

				353.44		1.177353

				353.46		1.177353

				353.49		1.177353

				353.51		1.177353

				353.53		1.177353

				353.55		1.177353

				353.57		1.177353

				353.59		1.177353

				353.61		1.177353

				353.63		1.177353

				353.66		1.177353

				353.68		1.171582

				353.7		1.177353

				353.72		1.177353

				353.74		1.177353

				353.76		1.177353

				353.78		1.177353

				353.8		1.177353

				353.82		1.177353

				353.85		1.177353

				353.87		1.177353

				353.89		1.177353

				353.91		1.171582

				353.93		1.177353

				353.95		1.171582

				353.97		1.171582

				353.99		1.171582

				354.02		1.171582

				354.04		1.171582

				354.06		1.171582

				354.08		1.171582

				354.1		1.171582

				354.12		1.171582

				354.14		1.171582

				354.16		1.171582

				354.19		1.171582

				354.21		1.177353

				354.23		1.171582

				354.25		1.171582

				354.27		1.171582

				354.29		1.171582

				354.31		1.171582

				354.33		1.171582

				354.36		1.171582

				354.38		1.171582

				354.4		1.171582

				354.42		1.171582

				354.44		1.171582

				354.46		1.171582

				354.48		1.171582

				354.5		1.171582

				354.52		1.171582

				354.55		1.171582

				354.57		1.171582

				354.59		1.171582

				354.61		1.171582

				354.63		1.171582

				354.65		1.171582

				354.67		1.171582

				354.69		1.171582

				354.72		1.171582

				354.74		1.165811

				354.76		1.165811

				354.78		1.165811

				354.8		1.165811

				354.82		1.165811

				354.84		1.165811

				354.86		1.165811

				354.89		1.165811

				354.91		1.165811

				354.93		1.165811

				354.95		1.171582

				354.97		1.165811

				354.99		1.165811

				355.01		1.165811

				355.03		1.171582

				355.05		1.165811

				355.08		1.165811

				355.1		1.165811

				355.12		1.165811

				355.14		1.165811

				355.16		1.165811

				355.18		1.165811

				355.2		1.165811

				355.22		1.165811

				355.25		1.165811

				355.27		1.165811

				355.29		1.165811

				355.31		1.165811

				355.33		1.165811

				355.35		1.165811

				355.37		1.165811

				355.39		1.165811

				355.42		1.165811

				355.44		1.165811

				355.46		1.165811

				355.48		1.165811

				355.5		1.165811

				355.52		1.165811

				355.54		1.165811

				355.56		1.165811

				355.59		1.165811

				355.61		1.165811

				355.63		1.165811

				355.65		1.165811

				355.67		1.165811

				355.69		1.171582

				355.71		1.171582

				355.73		1.171582

				355.76		1.171582

				355.78		1.171582

				355.8		1.171582

				355.82		1.171582

				355.84		1.171582

				355.86		1.171582

				355.88		1.171582

				355.9		1.171582

				355.93		1.171582

				355.95		1.171582

				355.97		1.171582

				355.99		1.171582

				356.01		1.171582

				356.03		1.171582

				356.05		1.171582

				356.07		1.171582

				356.1		1.171582

				356.12		1.171582

				356.14		1.171582

				356.16		1.177353

				356.18		1.177353

				356.2		1.171582

				356.22		1.171582

				356.24		1.177353

				356.27		1.177353

				356.29		1.171582

				356.31		1.171582

				356.33		1.177353

				356.35		1.171582

				356.37		1.177353

				356.39		1.171582

				356.41		1.177353

				356.44		1.171582

				356.46		1.177353

				356.48		1.177353

				356.5		1.177353

				356.52		1.177353

				356.54		1.177353

				356.56		1.177353

				356.58		1.177353

				356.6		1.177353

				356.63		1.177353

				356.65		1.177353

				356.67		1.177353

				356.69		1.177353

				356.71		1.177353

				356.73		1.177353

				356.75		1.177353

				356.77		1.177353

				356.8		1.177353

				356.82		1.177353

				356.84		1.183125

				356.86		1.183125

				356.88		1.177353

				356.9		1.183125

				356.92		1.183125

				356.94		1.183125

				356.97		1.183125

				356.99		1.183125

				357.01		1.183125

				357.03		1.183125

				357.05		1.183125

				357.07		1.183125

				357.09		1.183125

				357.11		1.183125

				357.14		1.183125

				357.16		1.183125

				357.18		1.183125

				357.2		1.183125

				357.22		1.183125

				357.24		1.183125

				357.26		1.183125

				357.28		1.183125

				357.3		1.183125

				357.33		1.183125

				357.35		1.183125

				357.37		1.183125

				357.39		1.183125

				357.41		1.183125

				357.43		1.183125

				357.45		1.183125

				357.47		1.183125

				357.5		1.183125

				357.52		1.183125

				357.54		1.183125

				357.56		1.183125

				357.58		1.183125

				357.6		1.183125

				357.62		1.183125

				357.64		1.183125

				357.67		1.183125

				357.69		1.183125

				357.71		1.183125

				357.73		1.183125

				357.75		1.183125

				357.77		1.183125

				357.79		1.183125

				357.81		1.183125

				357.84		1.183125

				357.86		1.183125

				357.88		1.183125

				357.9		1.183125

				357.92		1.177353

				357.94		1.177353

				357.96		1.177353

				357.98		1.177353

				358		1.177353

				358.03		1.177353

				358.05		1.177353

				358.07		1.177353

				358.09		1.177353

				358.11		1.177353

				358.13		1.177353

				358.15		1.177353

				358.17		1.177353

				358.2		1.171582

				358.22		1.171582

				358.24		1.171582

				358.26		1.171582

				358.28		1.171582

				358.3		1.171582

				358.32		1.171582

				358.34		1.171582

				358.37		1.171582

				358.39		1.171582

				358.41		1.171582

				358.43		1.171582

				358.45		1.171582

				358.47		1.171582

				358.49		1.171582

				358.51		1.171582

				358.54		1.171582

				358.56		1.171582

				358.58		1.171582

				358.6		1.171582

				358.62		1.171582

				358.64		1.171582

				358.66		1.171582

				358.68		1.171582

				358.7		1.171582

				358.73		1.171582

				358.75		1.171582

				358.77		1.165811

				358.79		1.165811

				358.81		1.165811

				358.83		1.165811

				358.85		1.165811

				358.87		1.165811

				358.9		1.165811

				358.92		1.165811

				358.94		1.165811

				358.96		1.165811

				358.98		1.165811

				359		1.165811

				359.02		1.160039

				359.04		1.160039

				359.07		1.165811

				359.09		1.160039

				359.11		1.160039

				359.13		1.160039

				359.15		1.160039

				359.17		1.160039

				359.19		1.160039

				359.21		1.160039

				359.24		1.160039

				359.26		1.160039

				359.28		1.160039

				359.3		1.160039

				359.32		1.160039

				359.34		1.160039

				359.36		1.160039

				359.38		1.160039

				359.41		1.160039

				359.43		1.160039

				359.45		1.160039

				359.47		1.160039

				359.49		1.160039

				359.51		1.160039

				359.53		1.160039

				359.55		1.160039

				359.58		1.154268

				359.6		1.154268

				359.62		1.154268

				359.64		1.154268

				359.66		1.154268

				359.68		1.154268

				359.7		1.154268

				359.72		1.154268

				359.75		1.154268

				359.77		1.154268

				359.79		1.154268

				359.81		1.154268

				359.83		1.148497

				359.85		1.154268

				359.87		1.154268

				359.89		1.154268

				359.92		1.154268

				359.94		1.154268

				359.96		1.154268

				359.98		1.154268

				360		1.154268

				360.02		1.154268

				360.04		1.154268

				360.06		1.154268

				360.09		1.154268

				360.11		1.154268

				360.13		1.154268

				360.15		1.154268

				360.17		1.148497

				360.19		1.154268

				360.21		1.154268

				360.23		1.154268

				360.26		1.148497

				360.28		1.154268

				360.3		1.154268

				360.32		1.148497

				360.34		1.148497

				360.36		1.154268

				360.38		1.154268

				360.4		1.154268

				360.43		1.148497

				360.45		1.154268

				360.47		1.154268

				360.49		1.148497

				360.51		1.148497

				360.53		1.148497

				360.55		1.148497

				360.57		1.148497

				360.6		1.148497

				360.62		1.148497

				360.64		1.148497

				360.66		1.148497

				360.68		1.148497

				360.7		1.148497

				360.72		1.148497

				360.74		1.148497

				360.77		1.148497

				360.79		1.148497

				360.81		1.148497

				360.83		1.148497

				360.85		1.148497

				360.87		1.148497

				360.89		1.148497

				360.91		1.148497

				360.93		1.148497

				360.96		1.154268

				360.98		1.154268

				361		1.154268

				361.02		1.154268

				361.04		1.154268

				361.06		1.154268

				361.08		1.154268

				361.1		1.154268

				361.13		1.154268

				361.15		1.154268

				361.17		1.148497

				361.19		1.148497

				361.21		1.154268

				361.23		1.148497

				361.25		1.148497

				361.27		1.148497

				361.3		1.148497

				361.32		1.148497

				361.34		1.148497

				361.36		1.148497

				361.38		1.148497

				361.4		1.148497

				361.42		1.148497

				361.44		1.154268

				361.47		1.154268

				361.49		1.148497

				361.51		1.154268

				361.53		1.148497

				361.55		1.154268

				361.57		1.148497

				361.59		1.148497

				361.61		1.148497

				361.64		1.148497

				361.66		1.148497

				361.68		1.148497

				361.7		1.148497

				361.72		1.154268

				361.74		1.154268

				361.76		1.148497

				361.78		1.148497

				361.81		1.148497

				361.83		1.148497

				361.85		1.154268

				361.87		1.148497

				361.89		1.148497

				361.91		1.154268

				361.93		1.154268

				361.95		1.148497

				361.97		1.154268

				362		1.154268

				362.02		1.154268

				362.04		1.154268

				362.06		1.148497

				362.08		1.148497

				362.1		1.154268

				362.12		1.148497

				362.14		1.154268

				362.17		1.154268

				362.19		1.154268

				362.21		1.148497

				362.23		1.148497

				362.25		1.154268

				362.27		1.154268

				362.29		1.148497

				362.31		1.154268

				362.34		1.154268

				362.36		1.154268

				362.38		1.148497

				362.4		1.154268

				362.42		1.148497

				362.44		1.148497

				362.46		1.148497

				362.48		1.148497

				362.51		1.148497

				362.53		1.148497

				362.55		1.148497

				362.57		1.148497

				362.59		1.148497

				362.61		1.148497

				362.63		1.148497

				362.65		1.148497

				362.68		1.148497

				362.7		1.148497

				362.72		1.148497

				362.74		1.148497

				362.76		1.148497

				362.78		1.148497

				362.8		1.148497

				362.82		1.148497

				362.84		1.148497

				362.87		1.148497

				362.89		1.148497

				362.91		1.148497

				362.93		1.148497

				362.95		1.148497

				362.97		1.148497

				362.99		1.148497

				363.01		1.148497

				363.04		1.148497

				363.06		1.148497

				363.08		1.148497

				363.1		1.148497

				363.12		1.148497

				363.14		1.148497

				363.16		1.148497

				363.18		1.148497

				363.21		1.148497

				363.23		1.148497

				363.25		1.148497

				363.27		1.148497

				363.29		1.148497

				363.31		1.148497

				363.33		1.148497

				363.35		1.148497

				363.38		1.148497

				363.4		1.148497

				363.42		1.148497

				363.44		1.148497

				363.46		1.154268

				363.48		1.154268

				363.5		1.154268

				363.52		1.154268

				363.54		1.154268

				363.57		1.154268

				363.59		1.154268

				363.61		1.154268

				363.63		1.154268

				363.65		1.154268

				363.67		1.154268

				363.69		1.154268

				363.71		1.154268

				363.74		1.154268

				363.76		1.154268

				363.78		1.154268

				363.8		1.154268

				363.82		1.154268

				363.84		1.154268

				363.86		1.154268

				363.88		1.154268

				363.91		1.154268

				363.93		1.154268

				363.95		1.154268

				363.97		1.160039

				363.99		1.160039

				364.01		1.160039

				364.03		1.160039

				364.05		1.160039

				364.08		1.160039

				364.1		1.154268

				364.12		1.160039

				364.14		1.154268

				364.16		1.160039

				364.18		1.154268

				364.2		1.154268

				364.22		1.160039

				364.25		1.160039

				364.27		1.160039

				364.29		1.160039

				364.31		1.160039

				364.33		1.160039

				364.35		1.160039

				364.37		1.160039

				364.39		1.160039

				364.42		1.160039

				364.44		1.160039

				364.46		1.160039

				364.48		1.165811

				364.5		1.165811

				364.52		1.165811

				364.54		1.165811

				364.56		1.165811

				364.59		1.165811

				364.61		1.165811

				364.63		1.165811

				364.65		1.165811

				364.67		1.165811

				364.69		1.165811

				364.71		1.165811

				364.73		1.165811

				364.76		1.165811

				364.78		1.165811

				364.8		1.165811

				364.82		1.165811

				364.84		1.171582

				364.86		1.171582

				364.88		1.171582

				364.9		1.171582

				364.93		1.171582

				364.95		1.171582

				364.97		1.171582

				364.99		1.171582

				365.01		1.171582

				365.03		1.171582

				365.05		1.171582

				365.07		1.171582

				365.1		1.171582

				365.12		1.165811

				365.14		1.165811

				365.16		1.171582

				365.18		1.171582

				365.2		1.165811

				365.22		1.171582

				365.24		1.171582

				365.27		1.171582

				365.29		1.171582

				365.31		1.171582

				365.33		1.171582

				365.35		1.171582

				365.37		1.171582

				365.39		1.171582

				365.41		1.171582

				365.43		1.171582

				365.46		1.171582

				365.48		1.171582

				365.5		1.171582

				365.52		1.171582

				365.54		1.171582

				365.56		1.171582

				365.58		1.171582

				365.6		1.171582

				365.63		1.165811

				365.65		1.171582

				365.67		1.165811

				365.69		1.171582

				365.71		1.165811

				365.73		1.165811

				365.75		1.165811

				365.77		1.165811

				365.8		1.165811

				365.82		1.165811

				365.84		1.165811

				365.86		1.171582

				365.88		1.165811

				365.9		1.165811

				365.92		1.165811

				365.94		1.165811

				365.97		1.165811

				365.99		1.165811

				366.01		1.165811

				366.03		1.165811

				366.05		1.165811

				366.07		1.165811

				366.09		1.165811

				366.11		1.160039

				366.14		1.160039

				366.16		1.160039

				366.18		1.160039

				366.2		1.160039

				366.22		1.160039

				366.24		1.160039

				366.26		1.160039

				366.28		1.160039

				366.31		1.160039

				366.33		1.160039

				366.35		1.160039

				366.37		1.160039

				366.39		1.160039

				366.41		1.160039

				366.43		1.160039

				366.45		1.160039

				366.48		1.154268

				366.5		1.160039

				366.52		1.154268

				366.54		1.160039

				366.56		1.154268

				366.58		1.154268

				366.6		1.154268

				366.62		1.154268

				366.64		1.154268

				366.67		1.154268

				366.69		1.154268

				366.71		1.154268

				366.73		1.154268

				366.75		1.154268

				366.77		1.154268

				366.79		1.154268

				366.81		1.154268

				366.84		1.148497

				366.86		1.154268

				366.88		1.154268

				366.9		1.154268

				366.92		1.148497

				366.94		1.148497

				366.96		1.148497

				366.98		1.148497

				367.01		1.148497

				367.03		1.148497

				367.05		1.148497

				367.07		1.148497

				367.09		1.148497

				367.11		1.148497

				367.13		1.148497

				367.15		1.148497

				367.18		1.148497

				367.2		1.148497

				367.22		1.148497

				367.24		1.148497

				367.26		1.148497

				367.28		1.148497

				367.3		1.148497

				367.32		1.148497

				367.35		1.148497

				367.37		1.148497

				367.39		1.148497

				367.41		1.148497

				367.43		1.148497

				367.45		1.148497

				367.47		1.148497

				367.49		1.148497

				367.52		1.148497

				367.54		1.148497

				367.56		1.148497

				367.58		1.148497

				367.6		1.148497

				367.62		1.148497

				367.64		1.148497

				367.66		1.148497

				367.69		1.148497

				367.71		1.148497

				367.73		1.148497

				367.75		1.148497

				367.77		1.148497

				367.79		1.148497

				367.81		1.148497

				367.83		1.148497

				367.86		1.148497

				367.88		1.148497

				367.9		1.148497

				367.92		1.148497

				367.94		1.148497

				367.96		1.148497

				367.98		1.148497

				368		1.148497

				368.03		1.148497

				368.05		1.148497

				368.07		1.148497

				368.09		1.148497

				368.11		1.154268

				368.13		1.148497

				368.15		1.148497

				368.17		1.154268

				368.2		1.154268

				368.22		1.154268

				368.24		1.154268

				368.26		1.154268

				368.28		1.154268

				368.3		1.154268

				368.32		1.154268

				368.34		1.154268

				368.37		1.154268

				368.39		1.154268

				368.41		1.154268

				368.43		1.148497

				368.45		1.148497

				368.47		1.154268

				368.49		1.154268

				368.51		1.154268

				368.54		1.154268

				368.56		1.154268

				368.58		1.154268

				368.6		1.154268

				368.62		1.154268

				368.64		1.154268

				368.66		1.154268

				368.68		1.154268

				368.71		1.154268

				368.73		1.154268

				368.75		1.154268

				368.77		1.154268

				368.79		1.154268

				368.81		1.154268

				368.83		1.154268

				368.85		1.154268

				368.88		1.154268

				368.9		1.154268

				368.92		1.154268

				368.94		1.160039

				368.96		1.154268

				368.98		1.154268

				369		1.154268

				369.02		1.160039

				369.05		1.160039

				369.07		1.160039

				369.09		1.160039

				369.11		1.160039

				369.13		1.160039

				369.15		1.160039

				369.17		1.160039

				369.19		1.160039

				369.22		1.160039

				369.24		1.165811

				369.26		1.160039

				369.28		1.165811

				369.3		1.165811

				369.32		1.165811

				369.34		1.165811

				369.36		1.165811

				369.39		1.165811

				369.41		1.165811

				369.43		1.165811

				369.45		1.165811

				369.47		1.165811

				369.49		1.165811

				369.51		1.165811

				369.53		1.165811

				369.56		1.165811

				369.58		1.165811

				369.6		1.165811

				369.62		1.165811

				369.64		1.165811

				369.66		1.165811

				369.68		1.165811

				369.7		1.165811

				369.73		1.165811

				369.75		1.165811

				369.77		1.165811

				369.79		1.165811

				369.81		1.165811

				369.83		1.165811

				369.85		1.165811

				369.87		1.165811

				369.9		1.165811

				369.92		1.165811

				369.94		1.165811

				369.96		1.165811

				369.98		1.165811

				370		1.165811

				370.02		1.165811

				370.04		1.165811

				370.07		1.165811

				370.09		1.165811

				370.11		1.165811

				370.13		1.165811

				370.15		1.165811

				370.17		1.165811

				370.19		1.165811

				370.21		1.165811

				370.24		1.165811

				370.26		1.165811

				370.28		1.165811

				370.3		1.165811

				370.32		1.165811

				370.34		1.165811

				370.36		1.165811

				370.38		1.165811

				370.41		1.165811

				370.43		1.165811

				370.45		1.165811

				370.47		1.165811

				370.49		1.165811

				370.51		1.171582

				370.53		1.171582

				370.55		1.171582

				370.58		1.171582

				370.6		1.171582

				370.62		1.171582

				370.64		1.171582

				370.66		1.171582

				370.68		1.171582

				370.7		1.171582

				370.72		1.171582

				370.75		1.171582

				370.77		1.171582

				370.79		1.171582

				370.81		1.171582

				370.83		1.171582

				370.85		1.171582

				370.87		1.171582

				370.89		1.171582

				370.92		1.171582

				370.94		1.171582

				370.96		1.165811

				370.98		1.165811

				371		1.165811

				371.02		1.165811

				371.04		1.165811

				371.06		1.165811

				371.09		1.165811

				371.11		1.165811

				371.13		1.165811

				371.15		1.165811

				371.17		1.165811

				371.19		1.165811

				371.21		1.165811

				371.23		1.165811

				371.26		1.160039

				371.28		1.160039

				371.3		1.160039

				371.32		1.160039

				371.34		1.160039

				371.36		1.160039

				371.38		1.160039

				371.4		1.160039

				371.43		1.160039

				371.45		1.160039

				371.47		1.160039

				371.49		1.160039

				371.51		1.160039

				371.53		1.160039

				371.55		1.160039

				371.57		1.160039

				371.6		1.160039

				371.62		1.160039

				371.64		1.160039

				371.66		1.154268

				371.68		1.160039

				371.7		1.154268

				371.72		1.160039

				371.74		1.154268

				371.77		1.154268

				371.79		1.154268

				371.81		1.154268

				371.83		1.154268

				371.85		1.154268

				371.87		1.154268

				371.89		1.154268

				371.91		1.154268

				371.94		1.154268

				371.96		1.154268

				371.98		1.154268

				372		1.154268

				372.02		1.154268

				372.04		1.154268

				372.06		1.154268

				372.08		1.154268

				372.11		1.154268

				372.13		1.154268

				372.15		1.154268

				372.17		1.154268

				372.19		1.154268

				372.21		1.154268

				372.23		1.154268

				372.25		1.154268

				372.28		1.154268

				372.3		1.154268

				372.32		1.154268

				372.34		1.154268

				372.36		1.154268

				372.38		1.154268

				372.4		1.154268

				372.42		1.148497

				372.45		1.154268

				372.47		1.154268

				372.49		1.154268

				372.51		1.154268

				372.53		1.154268

				372.55		1.154268

				372.57		1.154268

				372.59		1.154268

				372.62		1.154268

				372.64		1.154268

				372.66		1.154268

				372.68		1.154268

				372.7		1.154268

				372.72		1.154268

				372.74		1.154268

				372.76		1.154268

				372.79		1.154268

				372.81		1.154268

				372.83		1.154268

				372.85		1.154268

				372.87		1.154268

				372.89		1.154268

				372.91		1.154268

				372.93		1.154268

				372.96		1.154268

				372.98		1.154268

				373		1.154268

				373.02		1.154268

				373.04		1.154268

				373.06		1.154268

				373.08		1.154268

				373.11		1.160039

				373.13		1.160039

				373.15		1.154268

				373.17		1.160039

				373.19		1.160039

				373.21		1.160039

				373.23		1.160039

				373.25		1.160039

				373.28		1.160039

				373.3		1.160039

				373.32		1.160039

				373.34		1.160039

				373.36		1.160039

				373.38		1.160039

				373.4		1.160039

				373.42		1.160039

				373.45		1.160039

				373.47		1.160039

				373.49		1.165811

				373.51		1.160039

				373.53		1.165811

				373.55		1.160039

				373.57		1.165811

				373.59		1.165811

				373.62		1.165811

				373.64		1.165811

				373.66		1.165811

				373.68		1.165811

				373.7		1.165811

				373.72		1.165811

				373.74		1.165811

				373.76		1.165811

				373.79		1.160039

				373.81		1.160039

				373.83		1.160039

				373.85		1.165811

				373.87		1.165811

				373.89		1.165811

				373.91		1.165811

				373.93		1.165811

				373.96		1.165811

				373.98		1.165811

				374		1.165811

				374.02		1.165811

				374.04		1.165811

				374.06		1.165811

				374.08		1.165811

				374.1		1.165811

				374.13		1.165811

				374.15		1.165811

				374.17		1.165811

				374.19		1.171582

				374.21		1.171582

				374.23		1.165811

				374.25		1.165811

				374.27		1.171582

				374.3		1.171582

				374.32		1.171582

				374.34		1.171582

				374.36		1.171582

				374.38		1.171582

				374.4		1.171582

				374.42		1.171582

				374.45		1.171582

				374.47		1.171582

				374.49		1.171582

				374.51		1.171582

				374.53		1.171582

				374.55		1.171582

				374.57		1.171582

				374.59		1.171582

				374.62		1.171582

				374.64		1.165811

				374.66		1.165811

				374.68		1.165811

				374.7		1.165811

				374.72		1.165811

				374.74		1.165811

				374.76		1.165811

				374.79		1.165811

				374.81		1.165811

				374.83		1.165811

				374.85		1.165811

				374.87		1.165811

				374.89		1.165811

				374.91		1.165811

				374.93		1.165811

				374.96		1.171582

				374.98		1.165811

				375		1.171582

				375.02		1.165811

				375.04		1.171582

				375.06		1.171582

				375.08		1.171582

				375.1		1.171582

				375.13		1.171582

				375.15		1.165811

				375.17		1.165811

				375.19		1.171582

				375.21		1.165811

				375.23		1.165811

				375.25		1.171582

				375.28		1.165811

				375.3		1.165811

				375.32		1.165811

				375.34		1.165811

				375.36		1.165811

				375.38		1.165811

				375.4		1.171582

				375.42		1.171582

				375.45		1.171582

				375.47		1.171582

				375.49		1.171582

				375.51		1.171582

				375.53		1.171582

				375.55		1.171582

				375.57		1.171582

				375.59		1.171582

				375.62		1.171582

				375.64		1.171582

				375.66		1.171582

				375.68		1.171582

				375.7		1.171582

				375.72		1.171582

				375.74		1.171582

				375.76		1.171582

				375.79		1.171582

				375.81		1.171582

				375.83		1.171582

				375.85		1.171582

				375.87		1.171582

				375.89		1.171582

				375.91		1.177353

				375.93		1.177353

				375.96		1.177353

				375.98		1.177353

				376		1.171582

				376.02		1.177353

				376.04		1.177353

				376.06		1.177353

				376.08		1.177353

				376.1		1.177353

				376.13		1.177353

				376.15		1.177353

				376.17		1.177353

				376.19		1.177353

				376.21		1.177353

				376.23		1.177353

				376.25		1.177353

				376.27		1.177353

				376.3		1.177353

				376.32		1.177353

				376.34		1.177353

				376.36		1.177353

				376.38		1.177353

				376.4		1.177353

				376.42		1.177353

				376.45		1.177353

				376.47		1.177353

				376.49		1.177353

				376.51		1.177353

				376.53		1.177353

				376.55		1.177353

				376.57		1.177353

				376.59		1.177353

				376.62		1.177353

				376.64		1.177353

				376.66		1.177353

				376.68		1.177353

				376.7		1.177353

				376.72		1.177353

				376.74		1.177353

				376.76		1.177353

				376.79		1.177353

				376.81		1.177353

				376.83		1.177353

				376.85		1.177353

				376.87		1.177353

				376.89		1.177353

				376.91		1.177353

				376.93		1.177353

				376.96		1.177353

				376.98		1.177353

				377		1.177353

				377.02		1.177353

				377.04		1.177353

				377.06		1.177353

				377.08		1.177353

				377.1		1.177353

				377.13		1.177353

				377.15		1.177353

				377.17		1.177353

				377.19		1.177353

				377.21		1.177353

				377.23		1.177353

				377.25		1.171582

				377.27		1.177353

				377.3		1.171582

				377.32		1.177353

				377.34		1.177353

				377.36		1.177353

				377.38		1.177353

				377.4		1.177353

				377.42		1.177353

				377.44		1.177353

				377.47		1.177353

				377.49		1.171582

				377.51		1.171582

				377.53		1.171582

				377.55		1.171582

				377.57		1.171582

				377.59		1.171582

				377.61		1.171582

				377.64		1.171582

				377.66		1.171582

				377.68		1.171582

				377.7		1.171582

				377.72		1.171582

				377.74		1.171582

				377.76		1.171582

				377.78		1.171582

				377.81		1.171582

				377.83		1.171582

				377.85		1.171582

				377.87		1.171582

				377.89		1.171582

				377.91		1.171582

				377.93		1.171582

				377.95		1.171582

				377.98		1.165811

				378		1.165811

				378.02		1.165811

				378.04		1.165811

				378.06		1.165811

				378.08		1.165811

				378.1		1.165811

				378.12		1.165811

				378.15		1.165811

				378.17		1.165811

				378.19		1.165811

				378.21		1.165811

				378.23		1.165811

				378.25		1.165811

				378.27		1.160039

				378.29		1.165811

				378.32		1.160039

				378.34		1.165811

				378.36		1.160039

				378.38		1.160039

				378.4		1.160039

				378.42		1.160039

				378.44		1.160039

				378.47		1.160039

				378.49		1.160039

				378.51		1.160039

				378.53		1.160039

				378.55		1.160039

				378.57		1.160039

				378.59		1.160039

				378.61		1.160039

				378.64		1.160039

				378.66		1.160039

				378.68		1.154268

				378.7		1.154268

				378.72		1.160039

				378.74		1.154268

				378.76		1.154268

				378.78		1.154268

				378.81		1.160039

				378.83		1.154268

				378.85		1.154268

				378.87		1.154268

				378.89		1.154268

				378.91		1.154268

				378.93		1.154268

				378.95		1.154268

				378.98		1.154268

				379		1.154268

				379.02		1.154268

				379.04		1.154268

				379.06		1.154268

				379.08		1.154268

				379.1		1.154268

				379.12		1.154268

				379.15		1.154268

				379.17		1.154268

				379.19		1.154268

				379.21		1.154268

				379.23		1.154268

				379.25		1.148497

				379.27		1.154268

				379.29		1.148497

				379.32		1.154268

				379.34		1.148497

				379.36		1.154268

				379.38		1.154268

				379.4		1.154268

				379.42		1.148497

				379.44		1.148497

				379.46		1.148497

				379.49		1.148497

				379.51		1.148497

				379.53		1.148497

				379.55		1.148497

				379.57		1.154268

				379.59		1.154268

				379.61		1.148497

				379.63		1.154268

				379.66		1.154268

				379.68		1.154268

				379.7		1.154268

				379.72		1.154268

				379.74		1.154268

				379.76		1.154268

				379.78		1.154268

				379.8		1.154268

				379.83		1.154268

				379.85		1.154268

				379.87		1.154268

				379.89		1.154268

				379.91		1.154268

				379.93		1.154268

				379.95		1.154268

				379.97		1.154268

				380		1.154268

				380.02		1.154268

				380.04		1.154268

				380.06		1.154268

				380.08		1.154268

				380.1		1.154268

				380.12		1.154268

				380.14		1.154268

				380.17		1.154268

				380.19		1.154268

				380.21		1.154268

				380.23		1.154268

				380.25		1.154268

				380.27		1.154268

				380.29		1.154268

				380.31		1.154268

				380.34		1.154268

				380.36		1.154268

				380.38		1.154268

				380.4		1.154268

				380.42		1.154268

				380.44		1.154268

				380.46		1.154268

				380.48		1.154268

				380.51		1.154268

				380.53		1.154268

				380.55		1.154268

				380.57		1.154268

				380.59		1.154268

				380.61		1.154268

				380.63		1.154268

				380.65		1.154268

				380.68		1.154268

				380.7		1.154268

				380.72		1.154268

				380.74		1.154268

				380.76		1.160039

				380.78		1.160039

				380.8		1.160039

				380.82		1.160039

				380.85		1.160039

				380.87		1.160039

				380.89		1.160039

				380.91		1.160039

				380.93		1.160039

				380.95		1.160039

				380.97		1.160039

				380.99		1.160039

				381.02		1.160039

				381.04		1.160039

				381.06		1.165811

				381.08		1.160039

				381.1		1.160039

				381.12		1.165811

				381.14		1.165811

				381.16		1.165811

				381.19		1.165811

				381.21		1.165811

				381.23		1.165811

				381.25		1.165811

				381.27		1.165811

				381.29		1.165811

				381.31		1.165811

				381.33		1.165811

				381.36		1.165811

				381.38		1.165811

				381.4		1.165811

				381.42		1.165811

				381.44		1.165811

				381.46		1.165811

				381.48		1.165811

				381.5		1.165811

				381.53		1.165811

				381.55		1.165811

				381.57		1.165811

				381.59		1.165811

				381.61		1.165811

				381.63		1.165811

				381.65		1.165811

				381.67		1.165811

				381.69		1.165811

				381.72		1.165811

				381.74		1.165811

				381.76		1.165811

				381.78		1.165811

				381.8		1.165811

				381.82		1.165811

				381.84		1.165811

				381.86		1.165811

				381.89		1.165811

				381.91		1.165811

				381.93		1.165811

				381.95		1.165811

				381.97		1.165811

				381.99		1.165811

				382.01		1.165811

				382.03		1.165811

				382.06		1.165811

				382.08		1.165811

				382.1		1.165811

				382.12		1.160039

				382.14		1.165811

				382.16		1.160039

				382.18		1.160039

				382.2		1.160039

				382.23		1.160039

				382.25		1.160039

				382.27		1.160039

				382.29		1.160039

				382.31		1.160039

				382.33		1.160039

				382.35		1.160039

				382.37		1.165811

				382.39		1.165811

				382.42		1.165811

				382.44		1.165811

				382.46		1.165811

				382.48		1.160039

				382.5		1.165811

				382.52		1.160039

				382.54		1.165811

				382.56		1.165811

				382.59		1.165811

				382.61		1.160039

				382.63		1.160039

				382.65		1.160039

				382.67		1.160039

				382.69		1.160039

				382.71		1.160039

				382.73		1.160039

				382.76		1.160039

				382.78		1.160039

				382.8		1.160039

				382.82		1.160039

				382.84		1.160039

				382.86		1.160039

				382.88		1.160039

				382.9		1.160039

				382.93		1.160039

				382.95		1.160039

				382.97		1.160039

				382.99		1.160039

				383.01		1.160039

				383.03		1.160039

				383.05		1.160039

				383.07		1.160039

				383.09		1.154268

				383.12		1.154268

				383.14		1.154268

				383.16		1.154268

				383.18		1.154268

				383.2		1.154268

				383.22		1.154268

				383.24		1.154268

				383.26		1.154268

				383.29		1.154268

				383.31		1.154268

				383.33		1.154268

				383.35		1.154268

				383.37		1.154268

				383.39		1.154268

				383.41		1.154268

				383.43		1.154268

				383.46		1.154268

				383.48		1.154268

				383.5		1.154268

				383.52		1.154268

				383.54		1.154268

				383.56		1.148497

				383.58		1.148497

				383.6		1.148497

				383.63		1.148497

				383.65		1.148497

				383.67		1.148497

				383.69		1.148497

				383.71		1.148497

				383.73		1.148497

				383.75		1.148497

				383.77		1.148497

				383.79		1.148497

				383.82		1.148497

				383.84		1.148497

				383.86		1.148497

				383.88		1.148497

				383.9		1.148497

				383.92		1.154268

				383.94		1.148497

				383.96		1.148497

				383.99		1.148497

				384.01		1.148497

				384.03		1.148497

				384.05		1.148497

				384.07		1.148497

				384.09		1.148497

				384.11		1.148497

				384.13		1.148497

				384.16		1.148497

				384.18		1.148497

				384.2		1.148497

				384.22		1.148497

				384.24		1.148497

				384.26		1.148497

				384.28		1.148497

				384.3		1.148497

				384.33		1.148497

				384.35		1.154268

				384.37		1.148497

				384.39		1.148497

				384.41		1.148497

				384.43		1.148497

				384.45		1.148497

				384.47		1.148497

				384.5		1.148497

				384.52		1.148497

				384.54		1.148497

				384.56		1.148497

				384.58		1.148497

				384.6		1.148497

				384.62		1.148497

				384.64		1.148497

				384.67		1.148497

				384.69		1.148497

				384.71		1.148497

				384.73		1.148497

				384.75		1.148497

				384.77		1.148497

				384.79		1.148497

				384.81		1.148497

				384.84		1.148497

				384.86		1.148497

				384.88		1.148497

				384.9		1.148497

				384.92		1.148497

				384.94		1.148497

				384.96		1.148497

				384.98		1.148497

				385.01		1.148497

				385.03		1.148497

				385.05		1.148497

				385.07		1.148497

				385.09		1.148497

				385.11		1.148497

				385.13		1.148497

				385.15		1.148497

				385.18		1.148497

				385.2		1.148497

				385.22		1.154268

				385.24		1.154268

				385.26		1.154268

				385.28		1.154268

				385.3		1.154268

				385.32		1.154268

				385.34		1.154268

				385.37		1.154268

				385.39		1.154268

				385.41		1.154268

				385.43		1.154268

				385.45		1.154268

				385.47		1.148497

				385.49		1.148497

				385.51		1.148497

				385.54		1.148497

				385.56		1.148497

				385.58		1.148497

				385.6		1.148497

				385.62		1.148497

				385.64		1.148497

				385.66		1.148497

				385.68		1.154268

				385.71		1.154268

				385.73		1.154268

				385.75		1.154268

				385.77		1.154268

				385.79		1.154268

				385.81		1.154268

				385.83		1.154268

				385.85		1.154268

				385.88		1.154268

				385.9		1.154268

				385.92		1.154268

				385.94		1.148497

				385.96		1.154268

				385.98		1.154268

				386		1.148497

				386.02		1.148497

				386.04		1.148497

				386.07		1.148497

				386.09		1.148497

				386.11		1.148497

				386.13		1.148497

				386.15		1.154268

				386.17		1.154268

				386.19		1.154268

				386.21		1.154268

				386.24		1.154268

				386.26		1.154268

				386.28		1.154268

				386.3		1.154268

				386.32		1.154268

				386.34		1.154268

				386.36		1.154268

				386.38		1.154268

				386.41		1.154268

				386.43		1.154268

				386.45		1.154268

				386.47		1.154268

				386.49		1.154268

				386.51		1.154268

				386.53		1.154268

				386.55		1.154268

				386.57		1.154268

				386.6		1.154268

				386.62		1.154268

				386.64		1.154268

				386.66		1.154268

				386.68		1.154268

				386.7		1.154268

				386.72		1.154268

				386.74		1.154268

				386.77		1.154268

				386.79		1.154268

				386.81		1.154268

				386.83		1.154268

				386.85		1.154268

				386.87		1.154268

				386.89		1.154268

				386.91		1.154268

				386.94		1.154268

				386.96		1.154268

				386.98		1.154268

				387		1.154268

				387.02		1.154268

				387.04		1.154268

				387.06		1.154268

				387.08		1.154268

				387.1		1.154268

				387.13		1.154268

				387.15		1.154268

				387.17		1.154268

				387.19		1.154268

				387.21		1.154268

				387.23		1.154268

				387.25		1.160039

				387.27		1.154268

				387.3		1.154268

				387.32		1.154268

				387.34		1.154268

				387.36		1.154268

				387.38		1.154268

				387.4		1.154268

				387.42		1.154268

				387.44		1.154268

				387.47		1.154268

				387.49		1.160039

				387.51		1.154268

				387.53		1.154268

				387.55		1.160039

				387.57		1.160039

				387.59		1.160039

				387.61		1.160039

				387.64		1.160039

				387.66		1.160039

				387.68		1.160039

				387.7		1.160039

				387.72		1.160039

				387.74		1.160039

				387.76		1.160039

				387.78		1.160039

				387.8		1.160039

				387.83		1.160039

				387.85		1.160039

				387.87		1.160039

				387.89		1.160039

				387.91		1.160039

				387.93		1.160039

				387.95		1.160039

				387.97		1.160039

				388		1.160039

				388.02		1.160039

				388.04		1.160039

				388.06		1.160039

				388.08		1.160039

				388.1		1.160039

				388.12		1.160039

				388.14		1.160039

				388.17		1.160039

				388.19		1.165811

				388.21		1.160039

				388.23		1.160039

				388.25		1.165811

				388.27		1.160039

				388.29		1.165811

				388.31		1.165811

				388.33		1.160039

				388.36		1.160039

				388.38		1.160039

				388.4		1.160039

				388.42		1.160039

				388.44		1.160039

				388.46		1.160039

				388.48		1.160039

				388.5		1.160039

				388.53		1.160039

				388.55		1.160039

				388.57		1.160039

				388.59		1.160039

				388.61		1.160039

				388.63		1.160039

				388.65		1.160039

				388.67		1.160039

				388.69		1.160039

				388.72		1.160039

				388.74		1.160039

				388.76		1.160039

				388.78		1.160039

				388.8		1.160039

				388.82		1.160039

				388.84		1.160039

				388.86		1.160039

				388.89		1.160039

				388.91		1.160039

				388.93		1.160039

				388.95		1.160039

				388.97		1.160039

				388.99		1.160039

				389.01		1.160039

				389.03		1.160039

				389.05		1.160039

				389.08		1.160039

				389.1		1.160039

				389.12		1.160039

				389.14		1.160039

				389.16		1.165811

				389.18		1.160039

				389.2		1.160039

				389.22		1.160039

				389.25		1.160039

				389.27		1.160039

				389.29		1.160039

				389.31		1.160039

				389.33		1.160039

				389.35		1.160039

				389.37		1.160039

				389.39		1.160039

				389.41		1.160039

				389.44		1.160039

				389.46		1.160039

				389.48		1.160039

				389.5		1.160039

				389.52		1.160039

				389.54		1.160039

				389.56		1.160039

				389.58		1.160039

				389.61		1.165811

				389.63		1.165811

				389.65		1.160039

				389.67		1.165811

				389.69		1.160039

				389.71		1.160039

				389.73		1.165811

				389.75		1.165811

				389.78		1.160039

				389.8		1.165811

				389.82		1.160039

				389.84		1.160039

				389.86		1.160039

				389.88		1.160039

				389.9		1.160039

				389.92		1.160039

				389.94		1.160039

				389.97		1.160039

				389.99		1.160039

				390.01		1.160039

				390.03		1.160039

				390.05		1.160039

				390.07		1.160039

				390.09		1.160039

				390.11		1.165811

				390.14		1.160039

				390.16		1.165811

				390.18		1.165811

				390.2		1.160039

				390.22		1.165811

				390.24		1.160039

				390.26		1.165811

				390.28		1.160039

				390.3		1.165811

				390.33		1.165811

				390.35		1.160039

				390.37		1.165811

				390.39		1.160039

				390.41		1.160039

				390.43		1.160039

				390.45		1.165811

				390.47		1.165811

				390.5		1.165811

				390.52		1.165811

				390.54		1.165811

				390.56		1.165811

				390.58		1.165811

				390.6		1.165811

				390.62		1.171582

				390.64		1.171582

				390.66		1.171582

				390.69		1.171582

				390.71		1.171582

				390.73		1.171582

				390.75		1.171582

				390.77		1.171582

				390.79		1.171582

				390.81		1.171582

				390.83		1.171582

				390.86		1.171582

				390.88		1.171582

				390.9		1.171582

				390.92		1.171582

				390.94		1.165811

				390.96		1.165811

				390.98		1.165811

				391		1.171582

				391.03		1.165811

				391.05		1.165811

				391.07		1.165811

				391.09		1.165811

				391.11		1.171582

				391.13		1.165811

				391.15		1.165811

				391.17		1.165811

				391.19		1.165811

				391.22		1.165811

				391.24		1.165811

				391.26		1.165811

				391.28		1.165811

				391.3		1.165811

				391.32		1.165811

				391.34		1.165811

				391.36		1.165811

				391.39		1.165811

				391.41		1.165811

				391.43		1.165811

				391.45		1.165811

				391.47		1.160039

				391.49		1.165811

				391.51		1.160039

				391.53		1.165811

				391.55		1.165811

				391.58		1.165811

				391.6		1.165811

				391.62		1.165811

				391.64		1.165811

				391.66		1.165811

				391.68		1.165811

				391.7		1.165811

				391.72		1.165811

				391.75		1.165811

				391.77		1.160039

				391.79		1.165811

				391.81		1.160039

				391.83		1.160039

				391.85		1.160039

				391.87		1.160039

				391.89		1.160039

				391.92		1.160039

				391.94		1.160039

				391.96		1.160039

				391.98		1.160039

				392		1.160039

				392.02		1.160039

				392.04		1.160039

				392.06		1.160039

				392.09		1.160039

				392.11		1.160039

				392.13		1.160039

				392.15		1.160039

				392.17		1.160039

				392.19		1.160039

				392.21		1.160039

				392.23		1.160039

				392.25		1.160039

				392.28		1.160039

				392.3		1.160039

				392.32		1.160039

				392.34		1.160039

				392.36		1.160039

				392.38		1.160039

				392.4		1.160039

				392.42		1.160039

				392.45		1.160039

				392.47		1.160039

				392.49		1.160039

				392.51		1.160039

				392.53		1.160039

				392.55		1.160039

				392.57		1.160039

				392.59		1.160039

				392.62		1.160039

				392.64		1.160039

				392.66		1.160039

				392.68		1.160039

				392.7		1.160039

				392.72		1.154268

				392.74		1.154268

				392.76		1.154268

				392.78		1.154268

				392.81		1.154268

				392.83		1.154268

				392.85		1.154268

				392.87		1.154268

				392.89		1.160039

				392.91		1.160039

				392.93		1.154268

				392.95		1.154268

				392.98		1.154268

				393		1.154268

				393.02		1.148497

				393.04		1.154268

				393.06		1.154268

				393.08		1.154268

				393.1		1.154268

				393.12		1.154268

				393.15		1.154268

				393.17		1.154268

				393.19		1.154268

				393.21		1.154268

				393.23		1.154268

				393.25		1.154268

				393.27		1.154268

				393.29		1.154268

				393.32		1.154268

				393.34		1.154268

				393.36		1.148497

				393.38		1.154268

				393.4		1.154268

				393.42		1.154268

				393.44		1.154268

				393.46		1.154268

				393.49		1.154268

				393.51		1.154268

				393.53		1.154268

				393.55		1.154268

				393.57		1.154268

				393.59		1.154268

				393.61		1.154268

				393.63		1.154268

				393.66		1.154268

				393.68		1.154268

				393.7		1.160039

				393.72		1.160039

				393.74		1.160039

				393.76		1.160039

				393.78		1.154268

				393.8		1.154268

				393.82		1.154268

				393.85		1.154268

				393.87		1.154268

				393.89		1.154268

				393.91		1.154268

				393.93		1.154268

				393.95		1.154268

				393.97		1.154268

				393.99		1.154268

				394.02		1.154268

				394.04		1.154268

				394.06		1.154268

				394.08		1.154268

				394.1		1.154268

				394.12		1.154268

				394.14		1.154268

				394.16		1.160039

				394.18		1.160039

				394.21		1.154268

				394.23		1.154268

				394.25		1.160039

				394.27		1.154268

				394.29		1.154268

				394.31		1.154268

				394.33		1.160039

				394.35		1.154268

				394.38		1.154268

				394.4		1.160039

				394.42		1.160039

				394.44		1.160039

				394.46		1.160039

				394.48		1.160039

				394.5		1.154268

				394.52		1.160039

				394.54		1.160039

				394.57		1.160039

				394.59		1.154268

				394.61		1.154268

				394.63		1.154268

				394.65		1.154268

				394.67		1.154268

				394.69		1.154268

				394.71		1.154268

				394.74		1.154268

				394.76		1.154268

				394.78		1.154268

				394.8		1.154268

				394.82		1.154268

				394.84		1.154268

				394.86		1.154268

				394.88		1.154268

				394.91		1.154268

				394.93		1.154268

				394.95		1.154268

				394.97		1.154268

				394.99		1.154268

				395.01		1.154268

				395.03		1.154268

				395.05		1.160039

				395.07		1.160039

				395.1		1.160039

				395.12		1.160039

				395.14		1.160039

				395.16		1.160039

				395.18		1.160039

				395.2		1.160039

				395.22		1.160039

				395.24		1.160039

				395.27		1.160039

				395.29		1.160039

				395.31		1.160039

				395.33		1.160039

				395.35		1.160039

				395.37		1.160039

				395.39		1.160039

				395.41		1.160039

				395.44		1.160039

				395.46		1.160039

				395.48		1.160039

				395.5		1.160039

				395.52		1.160039

				395.54		1.160039

				395.56		1.160039

				395.58		1.160039

				395.6		1.160039

				395.63		1.160039

				395.65		1.160039

				395.67		1.160039

				395.69		1.160039

				395.71		1.160039

				395.73		1.160039

				395.75		1.160039

				395.77		1.160039

				395.8		1.154268

				395.82		1.154268

				395.84		1.154268

				395.86		1.154268

				395.88		1.160039

				395.9		1.154268

				395.92		1.160039

				395.94		1.160039

				395.96		1.160039

				395.99		1.160039

				396.01		1.160039

				396.03		1.160039

				396.05		1.160039

				396.07		1.160039

				396.09		1.160039

				396.11		1.160039

				396.13		1.160039

				396.16		1.160039

				396.18		1.160039

				396.2		1.160039

				396.22		1.160039

				396.24		1.160039

				396.26		1.160039

				396.28		1.160039

				396.3		1.160039

				396.32		1.160039

				396.35		1.160039

				396.37		1.160039

				396.39		1.160039

				396.41		1.160039

				396.43		1.160039

				396.45		1.160039

				396.47		1.160039

				396.49		1.160039

				396.52		1.160039

				396.54		1.160039

				396.56		1.160039

				396.58		1.160039

				396.6		1.160039

				396.62		1.160039

				396.64		1.160039

				396.66		1.160039

				396.68		1.160039

				396.71		1.160039

				396.73		1.160039

				396.75		1.160039

				396.77		1.160039

				396.79		1.160039

				396.81		1.160039

				396.83		1.165811

				396.85		1.165811

				396.87		1.165811

				396.9		1.165811

				396.92		1.165811

				396.94		1.165811

				396.96		1.165811

				396.98		1.165811

				397		1.165811

				397.02		1.165811

				397.04		1.165811

				397.07		1.165811

				397.09		1.165811

				397.11		1.160039

				397.13		1.165811

				397.15		1.165811

				397.17		1.165811

				397.19		1.165811

				397.21		1.165811

				397.23		1.165811

				397.26		1.165811

				397.28		1.165811

				397.3		1.165811

				397.32		1.165811

				397.34		1.165811

				397.36		1.165811

				397.38		1.165811

				397.4		1.165811

				397.43		1.165811

				397.45		1.165811

				397.47		1.165811

				397.49		1.171582

				397.51		1.171582

				397.53		1.171582

				397.55		1.165811

				397.57		1.165811

				397.59		1.165811

				397.62		1.165811

				397.64		1.165811

				397.66		1.165811

				397.68		1.165811

				397.7		1.165811

				397.72		1.165811

				397.74		1.165811

				397.76		1.165811

				397.79		1.165811

				397.81		1.165811

				397.83		1.171582

				397.85		1.171582

				397.87		1.171582

				397.89		1.165811

				397.91		1.165811

				397.93		1.171582

				397.95		1.165811

				397.98		1.171582

				398		1.165811

				398.02		1.165811

				398.04		1.171582

				398.06		1.165811

				398.08		1.165811

				398.1		1.165811

				398.12		1.171582

				398.14		1.171582

				398.17		1.171582

				398.19		1.165811

				398.21		1.171582

				398.23		1.171582

				398.25		1.171582

				398.27		1.171582

				398.29		1.171582

				398.31		1.171582

				398.34		1.171582

				398.36		1.171582

				398.38		1.165811

				398.4		1.165811

				398.42		1.171582

				398.44		1.165811

				398.46		1.165811

				398.48		1.165811

				398.5		1.165811

				398.53		1.165811

				398.55		1.165811

				398.57		1.165811

				398.59		1.165811

				398.61		1.165811

				398.63		1.165811

				398.65		1.171582

				398.67		1.171582

				398.69		1.171582

				398.72		1.171582

				398.74		1.171582

				398.76		1.165811

				398.78		1.165811

				398.8		1.171582

				398.82		1.165811

				398.84		1.165811

				398.86		1.165811

				398.88		1.165811

				398.91		1.165811

				398.93		1.165811

				398.95		1.165811

				398.97		1.165811

				398.99		1.165811

				399.01		1.165811

				399.03		1.165811

				399.05		1.171582

				399.08		1.171582

				399.1		1.171582

				399.12		1.171582

				399.14		1.171582

				399.16		1.165811

				399.18		1.165811

				399.2		1.165811

				399.22		1.165811

				399.24		1.165811

				399.27		1.165811

				399.29		1.165811

				399.31		1.165811

				399.33		1.165811

				399.35		1.165811

				399.37		1.160039

				399.39		1.160039

				399.41		1.160039

				399.43		1.160039

				399.46		1.160039

				399.48		1.160039

				399.5		1.160039

				399.52		1.160039

				399.54		1.160039

				399.56		1.160039

				399.58		1.154268

				399.6		1.154268

				399.63		1.154268

				399.65		1.154268

				399.67		1.154268

				399.69		1.154268

				399.71		1.160039

				399.73		1.160039

				399.75		1.160039

				399.77		1.160039

				399.79		1.160039

				399.82		1.160039

				399.84		1.160039

				399.86		1.160039

				399.88		1.160039

				399.9		1.160039

				399.92		1.160039

				399.94		1.160039

				399.96		1.160039

				399.98		1.160039

				400.01		1.160039

				400.03		1.160039

				400.05		1.160039

				400.07		1.154268

				400.09		1.154268

				400.11		1.154268

				400.13		1.154268

				400.15		1.154268

				400.18		1.160039

				400.2		1.154268

				400.22		1.160039

				400.24		1.154268

				400.26		1.160039

				400.28		1.160039

				400.3		1.154268

				400.32		1.154268

				400.34		1.154268

				400.37		1.154268

				400.39		1.154268

				400.41		1.154268

				400.43		1.154268

				400.45		1.154268

				400.47		1.154268

				400.49		1.154268

				400.51		1.154268

				400.53		1.154268

				400.56		1.154268

				400.58		1.154268

				400.6		1.154268

				400.62		1.154268

				400.64		1.154268

				400.66		1.154268

				400.68		1.154268

				400.7		1.154268

				400.73		1.154268

				400.75		1.154268

				400.77		1.154268

				400.79		1.154268

				400.81		1.154268

				400.83		1.154268

				400.85		1.154268

				400.87		1.154268

				400.89		1.154268

				400.92		1.154268

				400.94		1.154268

				400.96		1.154268

				400.98		1.154268

				401		1.154268

				401.02		1.154268

				401.04		1.148497

				401.06		1.148497

				401.08		1.154268

				401.11		1.148497

				401.13		1.148497

				401.15		1.148497

				401.17		1.148497

				401.19		1.148497

				401.21		1.148497

				401.23		1.148497

				401.25		1.148497

				401.27		1.154268

				401.3		1.154268

				401.32		1.154268

				401.34		1.154268

				401.36		1.154268

				401.38		1.154268

				401.4		1.154268

				401.42		1.154268

				401.44		1.154268

				401.47		1.154268

				401.49		1.154268

				401.51		1.154268

				401.53		1.154268

				401.55		1.154268

				401.57		1.154268

				401.59		1.154268

				401.61		1.154268

				401.63		1.160039

				401.66		1.154268

				401.68		1.160039

				401.7		1.160039

				401.72		1.160039

				401.74		1.160039

				401.76		1.160039

				401.78		1.160039

				401.8		1.160039

				401.82		1.160039

				401.85		1.160039

				401.87		1.160039

				401.89		1.160039

				401.91		1.154268

				401.93		1.160039

				401.95		1.160039

				401.97		1.160039

				401.99		1.154268

				402.02		1.160039

				402.04		1.160039

				402.06		1.160039

				402.08		1.160039

				402.1		1.160039

				402.12		1.160039

				402.14		1.160039

				402.16		1.160039

				402.18		1.160039

				402.21		1.160039

				402.23		1.160039

				402.25		1.160039

				402.27		1.165811

				402.29		1.165811

				402.31		1.165811

				402.33		1.165811

				402.35		1.165811

				402.37		1.165811

				402.4		1.165811

				402.42		1.165811

				402.44		1.165811

				402.46		1.165811

				402.48		1.165811

				402.5		1.165811

				402.52		1.165811

				402.54		1.165811

				402.56		1.165811

				402.59		1.165811

				402.61		1.165811

				402.63		1.165811

				402.65		1.165811

				402.67		1.165811

				402.69		1.165811

				402.71		1.165811

				402.73		1.165811

				402.75		1.165811

				402.78		1.165811

				402.8		1.165811

				402.82		1.165811

				402.84		1.165811

				402.86		1.165811

				402.88		1.171582

				402.9		1.171582

				402.92		1.165811

				402.94		1.171582

				402.97		1.171582

				402.99		1.171582

				403.01		1.171582

				403.03		1.171582

				403.05		1.171582

				403.07		1.171582

				403.09		1.171582

				403.11		1.171582

				403.13		1.171582

				403.16		1.171582

				403.18		1.171582

				403.2		1.171582

				403.22		1.171582

				403.24		1.171582

				403.26		1.171582

				403.28		1.171582

				403.3		1.171582

				403.32		1.171582

				403.35		1.171582

				403.37		1.171582

				403.39		1.171582

				403.41		1.171582

				403.43		1.171582

				403.45		1.171582

				403.47		1.171582

				403.49		1.171582

				403.51		1.171582

				403.54		1.171582

				403.56		1.171582

				403.58		1.171582

				403.6		1.171582

				403.62		1.171582

				403.64		1.171582

				403.66		1.171582

				403.68		1.171582

				403.7		1.171582

				403.73		1.171582

				403.75		1.171582

				403.77		1.171582

				403.79		1.171582

				403.81		1.171582

				403.83		1.171582

				403.85		1.171582

				403.87		1.171582

				403.89		1.171582

				403.92		1.171582

				403.94		1.171582

				403.96		1.171582

				403.98		1.171582

				404		1.171582

				404.02		1.171582

				404.04		1.171582

				404.06		1.171582

				404.08		1.171582

				404.11		1.171582

				404.13		1.171582

				404.15		1.171582

				404.17		1.171582

				404.19		1.171582

				404.21		1.171582

				404.23		1.171582

				404.25		1.171582

				404.27		1.171582

				404.3		1.171582

				404.32		1.171582

				404.34		1.171582

				404.36		1.171582

				404.38		1.171582

				404.4		1.171582

				404.42		1.171582

				404.44		1.171582

				404.46		1.171582

				404.49		1.171582

				404.51		1.177353

				404.53		1.177353

				404.55		1.177353

				404.57		1.177353

				404.59		1.177353

				404.61		1.177353

				404.63		1.177353

				404.65		1.177353

				404.68		1.177353

				404.7		1.177353

				404.72		1.177353

				404.74		1.177353

				404.76		1.177353

				404.78		1.177353

				404.8		1.177353

				404.82		1.177353

				404.84		1.177353

				404.87		1.183125

				404.89		1.183125

				404.91		1.183125

				404.93		1.177353

				404.95		1.177353

				404.97		1.177353

				404.99		1.177353

				405.01		1.183125

				405.03		1.177353

				405.06		1.177353

				405.08		1.177353

				405.1		1.183125

				405.12		1.177353

				405.14		1.177353

				405.16		1.177353

				405.18		1.183125

				405.2		1.177353

				405.22		1.177353

				405.24		1.177353

				405.27		1.177353

				405.29		1.183125

				405.31		1.177353

				405.33		1.183125

				405.35		1.183125

				405.37		1.183125

				405.39		1.183125

				405.41		1.183125

				405.43		1.183125

				405.46		1.183125

				405.48		1.183125

				405.5		1.183125

				405.52		1.183125

				405.54		1.183125

				405.56		1.183125

				405.58		1.183125

				405.6		1.183125

				405.62		1.183125

				405.64		1.183125

				405.67		1.183125

				405.69		1.183125

				405.71		1.183125

				405.73		1.183125

				405.75		1.183125

				405.77		1.183125

				405.79		1.183125

				405.81		1.183125

				405.83		1.188896

				405.85		1.183125

				405.88		1.183125

				405.9		1.183125

				405.92		1.183125

				405.94		1.183125

				405.96		1.183125

				405.98		1.183125

				406		1.183125

				406.02		1.183125

				406.04		1.183125

				406.06		1.183125

				406.09		1.183125

				406.11		1.183125

				406.13		1.183125

				406.15		1.183125

				406.17		1.183125

				406.19		1.183125

				406.21		1.183125

				406.23		1.183125

				406.25		1.183125

				406.27		1.183125

				406.3		1.183125

				406.32		1.183125

				406.34		1.183125

				406.36		1.183125

				406.38		1.183125

				406.4		1.183125

				406.42		1.183125

				406.44		1.183125

				406.46		1.183125

				406.48		1.183125

				406.51		1.183125

				406.53		1.183125

				406.55		1.183125

				406.57		1.183125

				406.59		1.183125

				406.61		1.183125

				406.63		1.183125

				406.65		1.183125

				406.67		1.183125

				406.69		1.183125

				406.72		1.183125

				406.74		1.183125

				406.76		1.183125

				406.78		1.177353

				406.8		1.183125

				406.82		1.183125

				406.84		1.177353

				406.86		1.177353

				406.88		1.183125

				406.9		1.177353

				406.92		1.177353

				406.95		1.183125

				406.97		1.177353

				406.99		1.183125

				407.01		1.183125

				407.03		1.183125

				407.05		1.183125

				407.07		1.183125

				407.09		1.183125

				407.11		1.183125

				407.13		1.183125

				407.16		1.183125

				407.18		1.183125

				407.2		1.183125

				407.22		1.183125

				407.24		1.183125

				407.26		1.183125

				407.28		1.183125

				407.3		1.183125

				407.32		1.183125

				407.34		1.183125

				407.36		1.183125

				407.39		1.183125

				407.41		1.183125

				407.43		1.183125

				407.45		1.183125

				407.47		1.183125

				407.49		1.183125

				407.51		1.183125

				407.53		1.177353

				407.55		1.183125

				407.57		1.183125

				407.6		1.183125

				407.62		1.183125

				407.64		1.183125

				407.66		1.183125

				407.68		1.183125

				407.7		1.183125

				407.72		1.183125

				407.74		1.183125

				407.76		1.183125

				407.78		1.177353

				407.81		1.183125

				407.83		1.177353

				407.85		1.177353

				407.87		1.177353

				407.89		1.183125

				407.91		1.177353

				407.93		1.177353

				407.95		1.177353

				407.97		1.183125

				407.99		1.183125

				408.02		1.183125

				408.04		1.177353

				408.06		1.183125

				408.08		1.183125

				408.1		1.183125

				408.12		1.183125

				408.14		1.183125

				408.16		1.183125

				408.18		1.183125

				408.2		1.183125

				408.23		1.183125

				408.25		1.183125

				408.27		1.183125

				408.29		1.183125

				408.31		1.183125

				408.33		1.183125

				408.35		1.183125

				408.37		1.177353

				408.39		1.177353

				408.41		1.177353

				408.44		1.177353

				408.46		1.177353

				408.48		1.177353

				408.5		1.177353

				408.52		1.177353

				408.54		1.177353

				408.56		1.177353

				408.58		1.177353

				408.6		1.177353

				408.62		1.177353

				408.65		1.177353

				408.67		1.177353

				408.69		1.177353

				408.71		1.177353

				408.73		1.177353

				408.75		1.177353

				408.77		1.177353

				408.79		1.177353

				408.81		1.177353

				408.83		1.177353

				408.86		1.177353

				408.88		1.177353

				408.9		1.177353

				408.92		1.177353

				408.94		1.177353

				408.96		1.177353

				408.98		1.177353

				409		1.177353

				409.02		1.177353

				409.05		1.177353

				409.07		1.177353

				409.09		1.177353

				409.11		1.177353

				409.13		1.177353

				409.15		1.177353

				409.17		1.177353

				409.19		1.177353

				409.21		1.177353

				409.23		1.177353

				409.26		1.177353

				409.28		1.177353

				409.3		1.177353

				409.32		1.177353

				409.34		1.177353

				409.36		1.171582

				409.38		1.171582

				409.4		1.171582

				409.42		1.171582

				409.44		1.171582

				409.47		1.171582

				409.49		1.177353

				409.51		1.171582

				409.53		1.171582

				409.55		1.171582

				409.57		1.177353

				409.59		1.177353

				409.61		1.177353

				409.63		1.177353

				409.65		1.171582

				409.68		1.171582

				409.7		1.171582

				409.72		1.171582

				409.74		1.171582

				409.76		1.177353

				409.78		1.171582

				409.8		1.171582

				409.82		1.177353

				409.84		1.177353

				409.86		1.177353

				409.89		1.171582

				409.91		1.177353

				409.93		1.171582

				409.95		1.171582

				409.97		1.171582

				409.99		1.171582

				410.01		1.177353

				410.03		1.171582

				410.05		1.177353

				410.07		1.171582

				410.1		1.171582

				410.12		1.171582

				410.14		1.171582

				410.16		1.171582

				410.18		1.171582

				410.2		1.171582

				410.22		1.171582

				410.24		1.171582

				410.26		1.171582

				410.28		1.171582

				410.3		1.171582

				410.33		1.171582

				410.35		1.171582

				410.37		1.171582

				410.39		1.171582

				410.41		1.171582

				410.43		1.171582

				410.45		1.171582

				410.47		1.171582

				410.49		1.154268

				410.51		1.154268

				410.54		1.154268

				410.56		1.154268

				410.58		1.131183

				410.6		1.131183

				410.62		1.131183

				410.64		1.125411

				410.66		1.125411

				410.68		1.125411

				410.7		1.125411

				410.72		1.11964

				410.75		1.11964

				410.77		1.11964

				410.79		1.125411

				410.81		1.125411

				410.83		1.125411

				410.85		1.125411

				410.87		1.125411

				410.89		1.125411

				410.91		1.125411

				410.93		1.125411

				410.96		1.125411

				410.98		1.131183

				411		1.131183

				411.02		1.131183

				411.04		1.131183

				411.06		1.131183

				411.08		1.131183

				411.1		1.131183

				411.12		1.136954

				411.14		1.136954

				411.16		1.136954

				411.19		1.136954

				411.21		1.136954

				411.23		1.131183

				411.25		1.131183

				411.27		1.131183

				411.29		1.131183

				411.31		1.125411

				411.33		1.125411

				411.35		1.125411

				411.37		1.11964

				411.4		1.11964

				411.42		1.113869

				411.44		1.113869

				411.46		1.108097

				411.48		1.108097

				411.5		1.108097

				411.52		1.108097

				411.54		1.11964

				411.56		1.148497

				411.58		1.177353

				411.6		1.177353

				411.63		1.177353

				411.65		1.177353

				411.67		1.183125

				411.69		1.183125

				411.71		1.194667

				411.73		1.194667

				411.75		1.194667

				411.77		1.194667

				411.79		1.194667

				411.81		1.194667

				411.83		1.194667

				411.86		1.194667

				411.88		1.200439

				411.9		1.200439

				411.92		1.200439

				411.94		1.200439

				411.96		1.200439

				411.98		1.200439

				412		1.200439

				412.02		1.20621

				412.04		1.200439

				412.06		1.200439

				412.09		1.200439

				412.11		1.200439

				412.13		1.200439

				412.15		1.200439

				412.17		1.200439

				412.19		1.200439

				412.21		1.200439

				412.23		1.200439

				412.25		1.200439

				412.27		1.200439

				412.3		1.20621

				412.32		1.20621

				412.34		1.20621

				412.36		1.20621

				412.38		1.20621

				412.4		1.20621

				412.42		1.200439

				412.44		1.20621

				412.46		1.20621

				412.48		1.20621

				412.51		1.20621

				412.53		1.20621

				412.55		1.20621

				412.57		1.20621

				412.59		1.20621

				412.61		1.20621

				412.63		1.200439

				412.65		1.20621

				412.67		1.200439

				412.69		1.200439

				412.71		1.200439

				412.74		1.200439

				412.76		1.20621

				412.78		1.20621

				412.8		1.20621

				412.82		1.20621

				412.84		1.20621

				412.86		1.20621

				412.88		1.211981

				412.9		1.229295

				412.92		1.235067

				412.95		1.235067

				412.97		1.240838

				412.99		1.240838

				413.01		1.240838

				413.03		1.240838

				413.05		1.240838

				413.07		1.235067

				413.09		1.235067

				413.11		1.235067

				413.13		1.229295

				413.16		1.229295

				413.18		1.229295

				413.2		1.229295

				413.22		1.223524

				413.24		1.223524

				413.26		1.223524

				413.28		1.223524

				413.3		1.223524

				413.32		1.223524

				413.34		1.217753

				413.37		1.223524

				413.39		1.217753

				413.41		1.217753

				413.43		1.217753

				413.45		1.217753

				413.47		1.217753

				413.49		1.217753

				413.51		1.217753

				413.53		1.217753

				413.55		1.217753

				413.58		1.217753

				413.6		1.217753

				413.62		1.217753

				413.64		1.217753

				413.66		1.217753

				413.68		1.217753

				413.7		1.217753

				413.72		1.217753

				413.74		1.217753

				413.77		1.217753

				413.79		1.217753

				413.81		1.217753

				413.83		1.217753

				413.85		1.223524

				413.87		1.217753

				413.89		1.223524

				413.91		1.223524

				413.93		1.223524

				413.96		1.223524

				413.98		1.223524

				414		1.223524

				414.02		1.223524

				414.04		1.229295

				414.06		1.229295

				414.08		1.223524

				414.1		1.217753

				414.12		1.217753

				414.15		1.211981

				414.17		1.217753

				414.19		1.217753

				414.21		1.217753

				414.23		1.20621

				414.25		1.194667

				414.27		1.188896

				414.29		1.188896

				414.31		1.188896

				414.34		1.188896

				414.36		1.188896

				414.38		1.183125

				414.4		1.177353

				414.42		1.177353

				414.44		1.177353

				414.46		1.183125

				414.48		1.177353

				414.5		1.183125

				414.52		1.177353

				414.55		1.177353

				414.57		1.177353

				414.59		1.183125

				414.61		1.183125

				414.63		1.183125

				414.65		1.183125

				414.67		1.177353

				414.69		1.177353

				414.71		1.183125

				414.74		1.177353

				414.76		1.183125

				414.78		1.183125

				414.8		1.183125

				414.82		1.183125

				414.84		1.183125

				414.86		1.183125

				414.88		1.183125

				414.9		1.183125

				414.92		1.183125

				414.95		1.183125

				414.97		1.183125

				414.99		1.183125

				415.01		1.183125

				415.03		1.183125

				415.05		1.183125

				415.07		1.183125

				415.09		1.188896

				415.11		1.183125

				415.14		1.188896

				415.16		1.188896

				415.18		1.188896

				415.2		1.188896

				415.22		1.188896

				415.24		1.188896

				415.26		1.188896

				415.28		1.188896

				415.3		1.188896

				415.32		1.188896

				415.35		1.188896

				415.37		1.188896

				415.39		1.188896

				415.41		1.188896

				415.43		1.188896

				415.45		1.188896

				415.47		1.188896

				415.49		1.188896

				415.51		1.188896

				415.53		1.188896

				415.56		1.188896

				415.58		1.188896

				415.6		1.188896

				415.62		1.188896

				415.64		1.188896

				415.66		1.188896

				415.68		1.188896

				415.7		1.194667

				415.72		1.194667

				415.75		1.194667

				415.77		1.194667

				415.79		1.194667

				415.81		1.194667

				415.83		1.194667

				415.85		1.194667

				415.87		1.194667

				415.89		1.194667

				415.91		1.194667

				415.93		1.194667

				415.96		1.194667

				415.98		1.194667

				416		1.194667

				416.02		1.194667

				416.04		1.194667

				416.06		1.194667

				416.08		1.194667

				416.1		1.194667

				416.12		1.194667

				416.14		1.194667

				416.17		1.194667

				416.19		1.194667

				416.21		1.194667

				416.23		1.194667

				416.25		1.194667

				416.27		1.194667

				416.29		1.194667

				416.31		1.194667

				416.33		1.194667

				416.36		1.194667

				416.38		1.194667

				416.4		1.194667

				416.42		1.194667

				416.44		1.194667

				416.46		1.194667

				416.48		1.194667

				416.5		1.194667

				416.52		1.194667

				416.54		1.194667

				416.57		1.194667

				416.59		1.194667

				416.61		1.194667

				416.63		1.200439

				416.65		1.200439

				416.67		1.200439

				416.69		1.200439

				416.71		1.194667

				416.73		1.188896

				416.75		1.183125

				416.78		1.177353

				416.8		1.177353

				416.82		1.177353

				416.84		1.177353

				416.86		1.177353

				416.88		1.177353

				416.9		1.177353

				416.92		1.177353

				416.94		1.177353

				416.96		1.177353

				416.99		1.171582

				417.01		1.171582

				417.03		1.171582

				417.05		1.171582

				417.07		1.171582

				417.09		1.171582

				417.11		1.165811

				417.13		1.171582

				417.15		1.171582

				417.17		1.171582

				417.2		1.165811

				417.22		1.165811

				417.24		1.165811

				417.26		1.165811

				417.28		1.165811

				417.3		1.165811

				417.32		1.165811

				417.34		1.165811

				417.36		1.165811

				417.38		1.165811

				417.41		1.171582

				417.43		1.165811

				417.45		1.171582

				417.47		1.171582

				417.49		1.171582

				417.51		1.177353

				417.53		1.171582

				417.55		1.177353

				417.57		1.188896

				417.59		1.194667

				417.62		1.200439

				417.64		1.20621

				417.66		1.20621

				417.68		1.20621

				417.7		1.20621

				417.72		1.20621

				417.74		1.20621

				417.76		1.20621

				417.78		1.20621

				417.8		1.20621

				417.83		1.20621

				417.85		1.20621

				417.87		1.20621

				417.89		1.200439

				417.91		1.20621

				417.93		1.200439

				417.95		1.20621

				417.97		1.20621

				417.99		1.20621

				418.01		1.20621

				418.03		1.20621

				418.06		1.20621

				418.08		1.20621

				418.1		1.20621

				418.12		1.20621

				418.14		1.20621

				418.16		1.20621

				418.18		1.20621

				418.2		1.20621

				418.22		1.20621

				418.24		1.20621

				418.26		1.200439

				418.29		1.229295

				418.31		1.246609

				418.33		1.252381

				418.35		1.258152

				418.37		1.263923

				418.39		1.269695

				418.41		1.275466

				418.43		1.281237

				418.45		1.281237

				418.47		1.275466

				418.5		1.269695

				418.52		1.269695

				418.54		1.263923

				418.56		1.263923

				418.58		1.258152

				418.6		1.258152

				418.62		1.252381

				418.64		1.252381

				418.66		1.246609

				418.68		1.246609

				418.71		1.246609

				418.73		1.246609

				418.75		1.240838

				418.77		1.240838

				418.79		1.240838

				418.81		1.240838

				418.83		1.240838

				418.85		1.235067

				418.87		1.240838

				418.89		1.240838

				418.92		1.240838

				418.94		1.240838

				418.96		1.240838

				418.98		1.240838

				419		1.240838

				419.02		1.240838

				419.04		1.246609

				419.06		1.240838

				419.08		1.229295

				419.11		1.223524

				419.13		1.211981

				419.15		1.20621

				419.17		1.211981

				419.19		1.200439

				419.21		1.200439

				419.23		1.200439

				419.25		1.194667

				419.27		1.194667

				419.29		1.194667

				419.32		1.194667

				419.34		1.194667

				419.36		1.194667

				419.38		1.194667

				419.4		1.194667

				419.42		1.194667

				419.44		1.194667

				419.46		1.194667

				419.48		1.194667

				419.51		1.194667

				419.53		1.194667

				419.55		1.194667

				419.57		1.194667

				419.59		1.194667

				419.61		1.194667

				419.63		1.194667

				419.65		1.194667

				419.67		1.188896

				419.69		1.188896

				419.72		1.188896

				419.74		1.188896

				419.76		1.188896

				419.78		1.188896

				419.8		1.194667

				419.82		1.188896

				419.84		1.194667

				419.86		1.194667

				419.88		1.194667

				419.9		1.194667

				419.93		1.194667

				419.95		1.194667

				419.97		1.194667

				419.99		1.194667

				420.01		1.194667

				420.03		1.194667

				420.05		1.194667

				420.07		1.194667

				420.09		1.194667

				420.11		1.188896

				420.14		1.188896

				420.16		1.188896

				420.18		1.188896

				420.2		1.188896

				420.22		1.188896

				420.24		1.188896

				420.26		1.188896

				420.28		1.188896

				420.3		1.188896

				420.32		1.188896

				420.35		1.188896

				420.37		1.188896

				420.39		1.188896

				420.41		1.188896

				420.43		1.188896

				420.45		1.188896

				420.47		1.188896

				420.49		1.188896

				420.51		1.188896

				420.54		1.188896

				420.56		1.188896

				420.58		1.188896

				420.6		1.188896

				420.62		1.188896

				420.64		1.188896

				420.66		1.188896

				420.68		1.188896

				420.7		1.188896

				420.72		1.188896

				420.75		1.188896

				420.77		1.188896

				420.79		1.188896

				420.81		1.188896

				420.83		1.188896

				420.85		1.188896

				420.87		1.188896

				420.89		1.188896

				420.91		1.188896

				420.93		1.188896

				420.96		1.188896

				420.98		1.188896

				421		1.188896

				421.02		1.188896

				421.04		1.188896

				421.06		1.188896

				421.08		1.188896

				421.1		1.188896

				421.12		1.188896

				421.14		1.188896

				421.17		1.188896

				421.19		1.188896

				421.21		1.188896

				421.23		1.188896

				421.25		1.188896

				421.27		1.188896

				421.29		1.188896

				421.31		1.188896

				421.33		1.188896

				421.35		1.188896

				421.38		1.188896

				421.4		1.188896

				421.42		1.188896

				421.44		1.188896

				421.46		1.188896

				421.48		1.188896

				421.5		1.188896

				421.52		1.188896

				421.54		1.188896

				421.56		1.188896

				421.59		1.188896

				421.61		1.188896

				421.63		1.188896

				421.65		1.188896

				421.67		1.188896

				421.69		1.188896

				421.71		1.188896

				421.73		1.188896

				421.75		1.183125

				421.77		1.188896

				421.8		1.183125

				421.82		1.188896

				421.84		1.183125

				421.86		1.188896

				421.88		1.183125

				421.9		1.183125

				421.92		1.183125

				421.94		1.183125

				421.96		1.183125

				421.98		1.183125

				422.01		1.183125

				422.03		1.183125

				422.05		1.183125

				422.07		1.183125

				422.09		1.183125

				422.11		1.183125

				422.13		1.183125

				422.15		1.183125

				422.17		1.183125

				422.19		1.183125

				422.22		1.188896

				422.24		1.188896

				422.26		1.188896

				422.28		1.188896

				422.3		1.188896

				422.32		1.188896

				422.34		1.188896

				422.36		1.188896

				422.38		1.188896

				422.4		1.188896

				422.42		1.188896

				422.45		1.188896

				422.47		1.188896

				422.49		1.188896

				422.51		1.188896

				422.53		1.188896

				422.55		1.188896

				422.57		1.188896

				422.59		1.188896

				422.61		1.188896

				422.63		1.188896

				422.66		1.188896

				422.68		1.188896

				422.7		1.188896

				422.72		1.188896

				422.74		1.188896

				422.76		1.188896

				422.78		1.188896

				422.8		1.188896

				422.82		1.188896

				422.84		1.188896

				422.87		1.188896

				422.89		1.188896

				422.91		1.188896

				422.93		1.188896

				422.95		1.188896

				422.97		1.188896

				422.99		1.188896

				423.01		1.188896

				423.03		1.188896

				423.05		1.188896

				423.08		1.188896

				423.1		1.188896

				423.12		1.188896

				423.14		1.188896

				423.16		1.188896

				423.18		1.188896

				423.2		1.188896

				423.22		1.183125

				423.24		1.188896

				423.26		1.183125

				423.28		1.183125

				423.31		1.188896

				423.33		1.183125

				423.35		1.188896

				423.37		1.188896

				423.39		1.188896

				423.41		1.188896

				423.43		1.188896

				423.45		1.188896

				423.47		1.188896

				423.49		1.188896

				423.51		1.188896

				423.54		1.188896

				423.56		1.188896

				423.58		1.188896

				423.6		1.188896

				423.62		1.188896

				423.64		1.188896

				423.66		1.188896

				423.68		1.188896

				423.7		1.188896

				423.72		1.188896

				423.75		1.188896

				423.77		1.188896

				423.79		1.188896

				423.81		1.188896

				423.83		1.194667

				423.85		1.188896

				423.87		1.194667

				423.89		1.194667

				423.91		1.194667

				423.93		1.194667

				423.95		1.194667

				423.98		1.194667

				424		1.194667

				424.02		1.194667

				424.04		1.194667

				424.06		1.194667

				424.08		1.194667

				424.1		1.194667

				424.12		1.194667

				424.14		1.194667

				424.16		1.194667

				424.18		1.194667

				424.21		1.194667

				424.23		1.194667

				424.25		1.194667

				424.27		1.194667

				424.29		1.194667

				424.31		1.194667

				424.33		1.194667

				424.35		1.194667

				424.37		1.194667

				424.39		1.194667

				424.41		1.194667

				424.44		1.194667

				424.46		1.194667

				424.48		1.194667

				424.5		1.194667

				424.52		1.194667

				424.54		1.194667

				424.56		1.194667

				424.58		1.194667

				424.6		1.194667

				424.62		1.194667

				424.64		1.194667

				424.67		1.194667

				424.69		1.200439

				424.71		1.194667

				424.73		1.194667

				424.75		1.194667

				424.77		1.194667

				424.79		1.194667

				424.81		1.194667

				424.83		1.194667

				424.85		1.194667

				424.87		1.200439

				424.9		1.200439

				424.92		1.200439

				424.94		1.200439

				424.96		1.200439

				424.98		1.200439

				425		1.200439

				425.02		1.200439

				425.04		1.200439

				425.06		1.200439

				425.08		1.200439

				425.11		1.20621

				425.13		1.200439

				425.15		1.200439

				425.17		1.20621

				425.19		1.20621

				425.21		1.20621

				425.23		1.20621

				425.25		1.20621

				425.27		1.20621

				425.29		1.211981

				425.31		1.20621

				425.34		1.211981

				425.36		1.20621

				425.38		1.211981

				425.4		1.211981

				425.42		1.211981

				425.44		1.20621

				425.46		1.20621

				425.48		1.20621

				425.5		1.20621

				425.52		1.211981

				425.54		1.20621

				425.57		1.211981

				425.59		1.211981

				425.61		1.211981

				425.63		1.20621

				425.65		1.20621

				425.67		1.211981

				425.69		1.20621

				425.71		1.20621

				425.73		1.20621

				425.75		1.20621

				425.77		1.20621

				425.8		1.20621

				425.82		1.20621

				425.84		1.20621

				425.86		1.20621

				425.88		1.20621

				425.9		1.20621

				425.92		1.20621

				425.94		1.20621

				425.96		1.20621

				425.98		1.20621

				426		1.20621

				426.03		1.20621

				426.05		1.20621

				426.07		1.20621

				426.09		1.20621

				426.11		1.20621

				426.13		1.20621

				426.15		1.20621

				426.17		1.20621

				426.19		1.20621

				426.21		1.20621

				426.23		1.200439

				426.26		1.20621

				426.28		1.200439

				426.3		1.20621

				426.32		1.200439

				426.34		1.20621

				426.36		1.20621

				426.38		1.20621

				426.4		1.20621

				426.42		1.20621

				426.44		1.20621

				426.46		1.20621

				426.49		1.20621

				426.51		1.20621

				426.53		1.20621

				426.55		1.20621

				426.57		1.20621

				426.59		1.20621

				426.61		1.20621

				426.63		1.20621

				426.65		1.20621

				426.67		1.20621

				426.69		1.20621

				426.72		1.20621

				426.74		1.20621

				426.76		1.20621

				426.78		1.20621

				426.8		1.20621

				426.82		1.20621

				426.84		1.20621

				426.86		1.20621

				426.88		1.20621

				426.9		1.20621

				426.92		1.20621

				426.95		1.20621

				426.97		1.20621

				426.99		1.20621

				427.01		1.20621

				427.03		1.20621

				427.05		1.20621

				427.07		1.20621

				427.09		1.20621

				427.11		1.20621

				427.13		1.20621

				427.15		1.20621

				427.18		1.20621

				427.2		1.20621

				427.22		1.20621

				427.24		1.20621

				427.26		1.200439

				427.28		1.20621

				427.3		1.20621

				427.32		1.20621

				427.34		1.20621

				427.36		1.20621

				427.39		1.20621

				427.41		1.20621

				427.43		1.20621

				427.45		1.20621

				427.47		1.20621

				427.49		1.20621

				427.51		1.20621

				427.53		1.200439

				427.55		1.200439

				427.57		1.20621

				427.59		1.20621

				427.62		1.20621

				427.64		1.200439

				427.66		1.200439

				427.68		1.200439

				427.7		1.200439

				427.72		1.200439

				427.74		1.200439

				427.76		1.200439

				427.78		1.200439

				427.8		1.200439

				427.82		1.20621

				427.85		1.20621

				427.87		1.200439

				427.89		1.200439

				427.91		1.200439

				427.93		1.200439

				427.95		1.200439

				427.97		1.200439

				427.99		1.200439

				428.01		1.200439

				428.03		1.200439

				428.05		1.200439

				428.08		1.200439

				428.1		1.200439

				428.12		1.20621

				428.14		1.200439

				428.16		1.20621

				428.18		1.20621

				428.2		1.20621

				428.22		1.20621

				428.24		1.20621

				428.26		1.20621

				428.28		1.211981

				428.31		1.211981

				428.33		1.20621

				428.35		1.217753

				428.37		1.211981

				428.39		1.211981

				428.41		1.211981

				428.43		1.211981

				428.45		1.20621

				428.47		1.20621

				428.49		1.20621

				428.51		1.20621

				428.54		1.20621

				428.56		1.20621

				428.58		1.20621

				428.6		1.20621

				428.62		1.20621

				428.64		1.20621

				428.66		1.20621

				428.68		1.20621

				428.7		1.20621

				428.72		1.20621

				428.74		1.20621

				428.77		1.20621

				428.79		1.211981

				428.81		1.20621

				428.83		1.20621

				428.85		1.20621

				428.87		1.20621

				428.89		1.20621

				428.91		1.20621

				428.93		1.20621

				428.95		1.20621

				428.97		1.20621

				429		1.20621

				429.02		1.20621

				429.04		1.20621

				429.06		1.20621

				429.08		1.20621

				429.1		1.20621

				429.12		1.20621

				429.14		1.20621

				429.16		1.20621

				429.18		1.20621

				429.2		1.20621

				429.23		1.20621

				429.25		1.20621

				429.27		1.20621

				429.29		1.20621

				429.31		1.20621

				429.33		1.20621

				429.35		1.20621

				429.37		1.20621

				429.39		1.20621

				429.41		1.20621

				429.43		1.20621

				429.46		1.20621

				429.48		1.20621

				429.5		1.20621

				429.52		1.20621

				429.54		1.20621

				429.56		1.20621

				429.58		1.20621

				429.6		1.20621

				429.62		1.20621

				429.64		1.20621

				429.66		1.20621

				429.69		1.20621

				429.71		1.20621

				429.73		1.20621

				429.75		1.20621

				429.77		1.20621

				429.79		1.20621

				429.81		1.20621

				429.83		1.20621

				429.85		1.20621

				429.87		1.20621

				429.89		1.20621

				429.92		1.20621

				429.94		1.20621

				429.96		1.20621

				429.98		1.20621

				430		1.20621

				430.02		1.20621

				430.04		1.20621

				430.06		1.20621

				430.08		1.20621

				430.1		1.20621

				430.12		1.20621

				430.15		1.20621

				430.17		1.20621

				430.19		1.20621

				430.21		1.20621

				430.23		1.20621

				430.25		1.20621

				430.27		1.20621

				430.29		1.20621

				430.31		1.20621

				430.33		1.200439

				430.36		1.200439

				430.38		1.200439

				430.4		1.200439

				430.42		1.200439

				430.44		1.200439

				430.46		1.200439

				430.48		1.200439

				430.5		1.200439

				430.52		1.20621

				430.54		1.20621

				430.56		1.20621

				430.59		1.20621

				430.61		1.20621

				430.63		1.20621

				430.65		1.20621

				430.67		1.200439

				430.69		1.200439

				430.71		1.200439

				430.73		1.200439

				430.75		1.200439

				430.77		1.200439

				430.79		1.200439

				430.82		1.200439

				430.84		1.200439

				430.86		1.200439

				430.88		1.200439

				430.9		1.200439

				430.92		1.200439

				430.94		1.200439

				430.96		1.200439

				430.98		1.200439

				431		1.200439

				431.02		1.200439

				431.05		1.200439

				431.07		1.200439

				431.09		1.200439

				431.11		1.200439

				431.13		1.200439

				431.15		1.200439

				431.17		1.200439

				431.19		1.20621

				431.21		1.200439

				431.23		1.20621

				431.26		1.20621

				431.28		1.20621

				431.3		1.20621

				431.32		1.20621

				431.34		1.20621

				431.36		1.200439

				431.38		1.200439

				431.4		1.200439

				431.42		1.200439

				431.44		1.200439

				431.46		1.200439

				431.49		1.200439

				431.51		1.200439

				431.53		1.200439

				431.55		1.200439

				431.57		1.200439

				431.59		1.200439

				431.61		1.200439

				431.63		1.200439

				431.65		1.200439

				431.67		1.200439

				431.69		1.200439

				431.72		1.200439

				431.74		1.200439

				431.76		1.200439

				431.78		1.200439

				431.8		1.200439

				431.82		1.200439

				431.84		1.200439

				431.86		1.200439

				431.88		1.200439

				431.9		1.200439

				431.92		1.200439

				431.95		1.20621

				431.97		1.200439

				431.99		1.20621

				432.01		1.20621

				432.03		1.20621

				432.05		1.20621

				432.07		1.20621

				432.09		1.20621

				432.11		1.20621

				432.13		1.20621

				432.15		1.20621

				432.18		1.20621

				432.2		1.20621

				432.22		1.20621

				432.24		1.20621

				432.26		1.20621

				432.28		1.20621

				432.3		1.20621

				432.32		1.20621

				432.34		1.20621

				432.36		1.20621

				432.38		1.20621

				432.41		1.211981

				432.43		1.211981

				432.45		1.211981

				432.47		1.211981

				432.49		1.211981

				432.51		1.211981

				432.53		1.211981

				432.55		1.211981

				432.57		1.211981

				432.59		1.211981

				432.61		1.211981

				432.64		1.211981

				432.66		1.211981

				432.68		1.211981

				432.7		1.211981

				432.72		1.211981

				432.74		1.211981

				432.76		1.211981

				432.78		1.211981

				432.8		1.211981

				432.82		1.211981

				432.84		1.211981

				432.87		1.211981

				432.89		1.211981

				432.91		1.211981

				432.93		1.211981

				432.95		1.211981

				432.97		1.211981

				432.99		1.211981

				433.01		1.211981

				433.03		1.211981

				433.05		1.211981

				433.07		1.211981

				433.1		1.211981

				433.12		1.211981

				433.14		1.217753

				433.16		1.217753

				433.18		1.217753

				433.2		1.217753

				433.22		1.217753

				433.24		1.211981

				433.26		1.217753

				433.28		1.217753

				433.3		1.211981

				433.33		1.211981

				433.35		1.217753

				433.37		1.217753

				433.39		1.211981

				433.41		1.217753

				433.43		1.217753

				433.45		1.217753

				433.47		1.217753

				433.49		1.217753

				433.51		1.217753

				433.54		1.217753

				433.56		1.217753

				433.58		1.217753

				433.6		1.217753

				433.62		1.217753

				433.64		1.223524

				433.66		1.217753

				433.68		1.223524

				433.7		1.223524

				433.72		1.223524

				433.74		1.223524

				433.77		1.223524

				433.79		1.223524

				433.81		1.223524

				433.83		1.223524

				433.85		1.223524

				433.87		1.223524

				433.89		1.223524

				433.91		1.229295

				433.93		1.223524

				433.95		1.223524

				433.97		1.229295

				434		1.223524

				434.02		1.229295

				434.04		1.229295

				434.06		1.229295

				434.08		1.229295

				434.1		1.223524

				434.12		1.229295

				434.14		1.223524

				434.16		1.223524

				434.18		1.223524

				434.2		1.223524

				434.23		1.223524

				434.25		1.223524

				434.27		1.223524

				434.29		1.223524

				434.31		1.223524

				434.33		1.223524

				434.35		1.223524

				434.37		1.223524

				434.39		1.223524

				434.41		1.223524

				434.44		1.223524

				434.46		1.223524

				434.48		1.223524

				434.5		1.223524

				434.52		1.223524

				434.54		1.223524

				434.56		1.223524

				434.58		1.223524

				434.6		1.223524

				434.62		1.223524

				434.64		1.223524

				434.67		1.223524

				434.69		1.223524

				434.71		1.223524

				434.73		1.223524

				434.75		1.223524

				434.77		1.223524

				434.79		1.223524

				434.81		1.223524

				434.83		1.223524

				434.85		1.223524

				434.87		1.223524

				434.9		1.223524

				434.92		1.223524

				434.94		1.223524

				434.96		1.223524

				434.98		1.229295

				435		1.229295

				435.02		1.223524

				435.04		1.229295

				435.06		1.229295

				435.08		1.229295

				435.1		1.223524

				435.13		1.223524

				435.15		1.223524

				435.17		1.223524

				435.19		1.223524

				435.21		1.223524

				435.23		1.223524

				435.25		1.223524

				435.27		1.223524

				435.29		1.223524

				435.31		1.223524

				435.33		1.223524

				435.36		1.223524

				435.38		1.223524

				435.4		1.223524

				435.42		1.223524

				435.44		1.223524

				435.46		1.229295

				435.48		1.223524

				435.5		1.223524

				435.52		1.223524

				435.54		1.223524

				435.57		1.223524

				435.59		1.223524

				435.61		1.223524

				435.63		1.223524

				435.65		1.223524

				435.67		1.223524

				435.69		1.223524

				435.71		1.223524

				435.73		1.223524

				435.75		1.223524

				435.77		1.223524

				435.8		1.223524

				435.82		1.223524

				435.84		1.223524

				435.86		1.223524

				435.88		1.223524

				435.9		1.223524

				435.92		1.223524

				435.94		1.217753

				435.96		1.217753

				435.98		1.217753

				436		1.217753

				436.03		1.217753

				436.05		1.217753

				436.07		1.217753

				436.09		1.217753

				436.11		1.217753

				436.13		1.223524

				436.15		1.217753

				436.17		1.217753

				436.19		1.217753

				436.21		1.223524

				436.23		1.217753

				436.26		1.217753

				436.28		1.223524

				436.3		1.223524

				436.32		1.223524

				436.34		1.223524

				436.36		1.223524

				436.38		1.223524

				436.4		1.223524

				436.42		1.223524

				436.44		1.223524

				436.47		1.223524

				436.49		1.223524

				436.51		1.223524

				436.53		1.223524

				436.55		1.223524

				436.57		1.223524

				436.59		1.223524

				436.61		1.223524

				436.63		1.223524

				436.65		1.223524

				436.67		1.223524

				436.7		1.223524

				436.72		1.223524

				436.74		1.223524

				436.76		1.223524

				436.78		1.223524

				436.8		1.223524

				436.82		1.223524

				436.84		1.223524

				436.86		1.223524

				436.88		1.223524

				436.9		1.229295

				436.93		1.223524

				436.95		1.229295

				436.97		1.229295

				436.99		1.223524

				437.01		1.229295

				437.03		1.223524

				437.05		1.229295

				437.07		1.223524

				437.09		1.223524

				437.11		1.229295

				437.13		1.229295

				437.16		1.223524

				437.18		1.229295

				437.2		1.229295

				437.22		1.229295

				437.24		1.229295

				437.26		1.229295

				437.28		1.229295

				437.3		1.229295

				437.32		1.229295

				437.34		1.229295

				437.36		1.229295

				437.39		1.229295

				437.41		1.229295

				437.43		1.229295

				437.45		1.229295

				437.47		1.229295

				437.49		1.229295

				437.51		1.229295

				437.53		1.229295

				437.55		1.235067

				437.57		1.235067

				437.59		1.235067

				437.62		1.235067

				437.64		1.235067

				437.66		1.235067

				437.68		1.235067

				437.7		1.235067

				437.72		1.235067

				437.74		1.235067

				437.76		1.235067

				437.78		1.235067

				437.8		1.235067

				437.83		1.235067

				437.85		1.235067

				437.87		1.235067

				437.89		1.235067

				437.91		1.235067

				437.93		1.235067

				437.95		1.235067

				437.97		1.235067

				437.99		1.235067

				438.01		1.235067

				438.03		1.235067

				438.06		1.235067

				438.08		1.235067

				438.1		1.235067

				438.12		1.235067

				438.14		1.235067

				438.16		1.240838

				438.18		1.235067

				438.2		1.235067

				438.22		1.235067

				438.24		1.240838

				438.26		1.240838

				438.29		1.240838

				438.31		1.240838

				438.33		1.240838

				438.35		1.240838

				438.37		1.240838

				438.39		1.240838

				438.41		1.235067

				438.43		1.235067

				438.45		1.235067

				438.47		1.240838

				438.49		1.235067

				438.52		1.240838

				438.54		1.240838

				438.56		1.240838

				438.58		1.235067

				438.6		1.240838

				438.62		1.240838

				438.64		1.240838

				438.66		1.240838

				438.68		1.240838

				438.7		1.240838

				438.72		1.240838

				438.75		1.240838

				438.77		1.240838

				438.79		1.240838

				438.81		1.240838

				438.83		1.240838

				438.85		1.240838

				438.87		1.240838

				438.89		1.240838

				438.91		1.240838

				438.93		1.240838

				438.95		1.240838

				438.98		1.240838

				439		1.240838

				439.02		1.240838

				439.04		1.246609

				439.06		1.246609

				439.08		1.246609

				439.1		1.246609

				439.12		1.246609

				439.14		1.246609

				439.16		1.246609

				439.19		1.246609

				439.21		1.246609

				439.23		1.246609

				439.25		1.246609

				439.27		1.246609

				439.29		1.246609

				439.31		1.246609

				439.33		1.246609

				439.35		1.246609

				439.37		1.246609

				439.39		1.246609

				439.42		1.246609

				439.44		1.246609

				439.46		1.246609

				439.48		1.246609

				439.5		1.246609

				439.52		1.246609

				439.54		1.246609

				439.56		1.246609

				439.58		1.246609

				439.6		1.246609

				439.62		1.246609

				439.65		1.246609

				439.67		1.246609

				439.69		1.246609

				439.71		1.246609

				439.73		1.246609

				439.75		1.246609

				439.77		1.246609

				439.79		1.246609

				439.81		1.246609

				439.83		1.246609

				439.85		1.246609

				439.88		1.246609

				439.9		1.246609

				439.92		1.246609

				439.94		1.246609

				439.96		1.246609

				439.98		1.246609

				440		1.246609

				440.02		1.246609

				440.04		1.246609

				440.06		1.246609

				440.08		1.246609

				440.11		1.246609

				440.13		1.246609

				440.15		1.246609

				440.17		1.246609

				440.19		1.246609

				440.21		1.252381

				440.23		1.246609

				440.25		1.252381

				440.27		1.246609

				440.29		1.252381

				440.31		1.252381

				440.34		1.246609

				440.36		1.252381

				440.38		1.246609

				440.4		1.246609

				440.42		1.252381

				440.44		1.252381

				440.46		1.252381

				440.48		1.252381

				440.5		1.252381

				440.52		1.252381

				440.54		1.252381

				440.57		1.252381

				440.59		1.252381

				440.61		1.252381

				440.63		1.252381

				440.65		1.252381

				440.67		1.252381

				440.69		1.252381

				440.71		1.252381

				440.73		1.252381

				440.75		1.252381

				440.78		1.252381

				440.8		1.252381

				440.82		1.252381

				440.84		1.252381

				440.86		1.252381

				440.88		1.252381

				440.9		1.252381

				440.92		1.252381

				440.94		1.246609

				440.96		1.246609

				440.98		1.246609

				441.01		1.252381

				441.03		1.246609

				441.05		1.252381

				441.07		1.252381

				441.09		1.252381

				441.11		1.246609

				441.13		1.252381

				441.15		1.246609

				441.17		1.246609

				441.19		1.246609

				441.21		1.246609

				441.24		1.246609

				441.26		1.246609

				441.28		1.246609

				441.3		1.246609

				441.32		1.246609

				441.34		1.246609

				441.36		1.246609

				441.38		1.246609

				441.4		1.246609

				441.42		1.246609

				441.45		1.246609

				441.47		1.246609

				441.49		1.246609

				441.51		1.246609

				441.53		1.240838

				441.55		1.240838

				441.57		1.240838

				441.59		1.246609

				441.61		1.246609

				441.63		1.246609

				441.65		1.240838

				441.68		1.246609

				441.7		1.246609

				441.72		1.246609

				441.74		1.240838

				441.76		1.246609

				441.78		1.246609

				441.8		1.246609

				441.82		1.246609

				441.84		1.246609

				441.86		1.246609

				441.88		1.246609

				441.91		1.246609

				441.93		1.246609

				441.95		1.246609

				441.97		1.246609

				441.99		1.246609

				442.01		1.246609

				442.03		1.246609

				442.05		1.246609

				442.07		1.246609

				442.09		1.246609

				442.12		1.246609

				442.14		1.246609

				442.16		1.246609

				442.18		1.246609

				442.2		1.246609

				442.22		1.246609

				442.24		1.246609

				442.26		1.246609

				442.28		1.240838

				442.3		1.240838

				442.32		1.240838

				442.35		1.240838

				442.37		1.240838

				442.39		1.240838

				442.41		1.240838

				442.43		1.240838

				442.45		1.240838

				442.47		1.240838

				442.49		1.240838

				442.51		1.240838

				442.53		1.240838

				442.55		1.240838

				442.58		1.240838

				442.6		1.240838

				442.62		1.240838

				442.64		1.240838

				442.66		1.240838

				442.68		1.240838

				442.7		1.240838

				442.72		1.240838

				442.74		1.240838

				442.76		1.240838

				442.79		1.240838

				442.81		1.240838

				442.83		1.240838

				442.85		1.240838

				442.87		1.240838

				442.89		1.240838

				442.91		1.240838

				442.93		1.240838

				442.95		1.240838

				442.97		1.240838

				442.99		1.240838

				443.02		1.240838

				443.04		1.240838

				443.06		1.240838

				443.08		1.240838

				443.1		1.240838

				443.12		1.240838

				443.14		1.240838

				443.16		1.240838

				443.18		1.246609

				443.2		1.240838

				443.22		1.240838

				443.25		1.240838

				443.27		1.240838

				443.29		1.240838

				443.31		1.240838

				443.33		1.240838

				443.35		1.240838

				443.37		1.240838

				443.39		1.240838

				443.41		1.240838

				443.43		1.240838

				443.46		1.240838

				443.48		1.240838

				443.5		1.240838

				443.52		1.240838

				443.54		1.240838

				443.56		1.240838

				443.58		1.240838

				443.6		1.246609

				443.62		1.246609

				443.64		1.246609

				443.66		1.246609

				443.69		1.246609

				443.71		1.246609

				443.73		1.246609

				443.75		1.246609

				443.77		1.240838

				443.79		1.240838

				443.81		1.240838

				443.83		1.240838

				443.85		1.240838

				443.87		1.240838

				443.89		1.240838

				443.92		1.240838

				443.94		1.240838

				443.96		1.240838

				443.98		1.240838

				444		1.240838

				444.02		1.240838

				444.04		1.240838

				444.06		1.240838

				444.08		1.246609

				444.1		1.240838

				444.13		1.246609

				444.15		1.246609

				444.17		1.246609

				444.19		1.246609

				444.21		1.240838

				444.23		1.240838

				444.25		1.246609

				444.27		1.240838

				444.29		1.240838

				444.31		1.240838

				444.33		1.240838

				444.36		1.240838

				444.38		1.240838

				444.4		1.240838

				444.42		1.246609

				444.44		1.246609

				444.46		1.246609

				444.48		1.246609

				444.5		1.246609

				444.52		1.246609

				444.54		1.246609

				444.57		1.246609

				444.59		1.246609

				444.61		1.246609

				444.63		1.246609

				444.65		1.246609

				444.67		1.240838

				444.69		1.246609

				444.71		1.240838

				444.73		1.240838

				444.75		1.240838

				444.77		1.240838

				444.8		1.240838

				444.82		1.246609

				444.84		1.246609

				444.86		1.246609

				444.88		1.246609

				444.9		1.246609

				444.92		1.246609

				444.94		1.246609

				444.96		1.246609

				444.98		1.246609

				445.01		1.246609

				445.03		1.246609

				445.05		1.246609

				445.07		1.246609

				445.09		1.246609

				445.11		1.246609

				445.13		1.246609

				445.15		1.246609

				445.17		1.246609

				445.19		1.246609

				445.22		1.246609

				445.24		1.246609

				445.26		1.246609

				445.28		1.246609

				445.3		1.246609

				445.32		1.246609

				445.34		1.246609

				445.36		1.246609

				445.38		1.246609

				445.4		1.246609

				445.42		1.246609

				445.45		1.246609

				445.47		1.252381

				445.49		1.252381

				445.51		1.252381

				445.53		1.252381

				445.55		1.252381

				445.57		1.252381

				445.59		1.252381

				445.61		1.252381

				445.63		1.252381

				445.66		1.252381

				445.68		1.252381

				445.7		1.252381

				445.72		1.252381

				445.74		1.252381

				445.76		1.252381

				445.78		1.252381

				445.8		1.252381

				445.82		1.252381

				445.84		1.258152

				445.86		1.252381

				445.89		1.258152

				445.91		1.258152

				445.93		1.258152

				445.95		1.258152

				445.97		1.252381

				445.99		1.258152

				446.01		1.258152

				446.03		1.258152

				446.05		1.258152

				446.07		1.258152

				446.1		1.258152

				446.12		1.258152

				446.14		1.258152

				446.16		1.258152

				446.18		1.258152

				446.2		1.258152

				446.22		1.258152

				446.24		1.258152

				446.26		1.258152

				446.28		1.258152

				446.3		1.258152

				446.33		1.258152

				446.35		1.258152

				446.37		1.258152

				446.39		1.258152

				446.41		1.258152

				446.43		1.258152

				446.45		1.258152

				446.47		1.258152

				446.49		1.258152

				446.51		1.258152

				446.53		1.258152

				446.56		1.258152

				446.58		1.258152

				446.6		1.258152

				446.62		1.258152

				446.64		1.258152

				446.66		1.258152

				446.68		1.258152

				446.7		1.258152

				446.72		1.258152

				446.74		1.258152

				446.77		1.258152

				446.79		1.258152

				446.81		1.258152

				446.83		1.258152

				446.85		1.258152

				446.87		1.258152

				446.89		1.258152

				446.91		1.258152

				446.93		1.258152

				446.95		1.258152

				446.97		1.258152

				447		1.258152

				447.02		1.258152

				447.04		1.258152

				447.06		1.258152

				447.08		1.258152

				447.1		1.258152

				447.12		1.258152

				447.14		1.258152

				447.16		1.258152

				447.18		1.258152

				447.21		1.258152

				447.23		1.258152

				447.25		1.258152

				447.27		1.258152

				447.29		1.258152

				447.31		1.258152

				447.33		1.258152

				447.35		1.258152

				447.37		1.258152

				447.39		1.258152

				447.42		1.258152

				447.44		1.258152

				447.46		1.258152

				447.48		1.258152

				447.5		1.258152

				447.52		1.258152

				447.54		1.258152

				447.56		1.258152

				447.58		1.252381

				447.6		1.252381

				447.62		1.252381

				447.65		1.252381

				447.67		1.252381

				447.69		1.252381

				447.71		1.252381

				447.73		1.252381

				447.75		1.252381

				447.77		1.252381

				447.79		1.252381

				447.81		1.252381

				447.83		1.252381

				447.86		1.252381

				447.88		1.252381

				447.9		1.252381

				447.92		1.246609

				447.94		1.252381

				447.96		1.246609

				447.98		1.246609

				448		1.252381

				448.02		1.246609

				448.04		1.246609

				448.07		1.246609

				448.09		1.246609

				448.11		1.246609

				448.13		1.246609

				448.15		1.246609

				448.17		1.246609

				448.19		1.246609

				448.21		1.246609

				448.23		1.246609

				448.25		1.246609

				448.27		1.246609

				448.3		1.246609

				448.32		1.246609

				448.34		1.246609

				448.36		1.246609

				448.38		1.246609

				448.4		1.246609

				448.42		1.246609

				448.44		1.246609

				448.46		1.246609

				448.48		1.246609

				448.51		1.246609

				448.53		1.246609

				448.55		1.246609

				448.57		1.246609

				448.59		1.246609

				448.61		1.252381

				448.63		1.252381

				448.65		1.252381

				448.67		1.252381

				448.69		1.252381

				448.72		1.246609

				448.74		1.252381

				448.76		1.252381

				448.78		1.252381

				448.8		1.252381

				448.82		1.252381

				448.84		1.252381

				448.86		1.252381

				448.88		1.252381

				448.9		1.252381

				448.93		1.252381

				448.95		1.252381

				448.97		1.252381

				448.99		1.252381

				449.01		1.252381

				449.03		1.252381

				449.05		1.252381

				449.07		1.246609

				449.09		1.252381

				449.11		1.246609

				449.14		1.252381

				449.16		1.252381

				449.18		1.252381

				449.2		1.252381

				449.22		1.252381

				449.24		1.252381

				449.26		1.252381

				449.28		1.252381

				449.3		1.252381

				449.32		1.252381

				449.35		1.252381

				449.37		1.252381

				449.39		1.252381

				449.41		1.252381

				449.43		1.252381

				449.45		1.252381

				449.47		1.252381

				449.49		1.252381

				449.51		1.252381

				449.53		1.252381

				449.56		1.252381

				449.58		1.252381

				449.6		1.252381

				449.62		1.252381

				449.64		1.252381

				449.66		1.252381

				449.68		1.252381

				449.7		1.252381

				449.72		1.252381

				449.74		1.252381

				449.77		1.252381

				449.79		1.252381

				449.81		1.252381

				449.83		1.252381

				449.85		1.252381

				449.87		1.252381

				449.89		1.252381

				449.91		1.252381

				449.93		1.252381

				449.95		1.252381

				449.97		1.258152

				450		1.258152

				450.02		1.258152

				450.04		1.258152

				450.06		1.258152

				450.08		1.258152

				450.1		1.258152

				450.12		1.258152

				450.14		1.258152

				450.16		1.258152

				450.18		1.258152

				450.21		1.258152

				450.23		1.258152

				450.25		1.258152

				450.27		1.258152

				450.29		1.258152

				450.31		1.258152

				450.33		1.258152

				450.35		1.263923

				450.37		1.263923

				450.39		1.263923

				450.42		1.263923

				450.44		1.263923

				450.46		1.263923

				450.48		1.263923

				450.5		1.263923

				450.52		1.263923

				450.54		1.263923

				450.56		1.263923

				450.58		1.263923

				450.6		1.263923

				450.62		1.263923

				450.65		1.263923

				450.67		1.263923

				450.69		1.263923

				450.71		1.258152

				450.73		1.263923

				450.75		1.258152

				450.77		1.258152

				450.79		1.258152

				450.81		1.258152

				450.83		1.263923

				450.86		1.263923

				450.88		1.258152

				450.9		1.252381

				450.92		1.246609

				450.94		1.240838

				450.96		1.240838

				450.98		1.240838

				451		1.240838

				451.02		1.240838

				451.04		1.240838

				451.06		1.240838

				451.09		1.240838

				451.11		1.240838

				451.13		1.240838

				451.15		1.235067

				451.17		1.235067

				451.19		1.235067

				451.21		1.235067

				451.23		1.235067

				451.25		1.235067

				451.27		1.235067

				451.3		1.235067

				451.32		1.235067

				451.34		1.235067

				451.36		1.229295

				451.38		1.223524

				451.4		1.223524

				451.42		1.217753

				451.44		1.217753

				451.46		1.217753

				451.48		1.217753

				451.51		1.217753

				451.53		1.217753

				451.55		1.217753

				451.57		1.217753

				451.59		1.217753

				451.61		1.223524

				451.63		1.223524

				451.65		1.229295

				451.67		1.229295

				451.69		1.229295

				451.71		1.240838

				451.74		1.246609

				451.76		1.258152

				451.78		1.263923

				451.8		1.269695

				451.82		1.269695

				451.84		1.269695

				451.86		1.269695

				451.88		1.263923

				451.9		1.269695

				451.92		1.263923

				451.94		1.263923

				451.97		1.263923

				451.99		1.263923

				452.01		1.263923

				452.03		1.263923

				452.05		1.263923

				452.07		1.263923

				452.09		1.263923

				452.11		1.263923

				452.13		1.263923

				452.15		1.263923

				452.17		1.263923

				452.2		1.263923

				452.22		1.263923

				452.24		1.263923

				452.26		1.263923

				452.28		1.263923

				452.3		1.263923

				452.32		1.263923

				452.34		1.263923

				452.36		1.263923

				452.38		1.263923

				452.4		1.263923

				452.43		1.263923

				452.45		1.281237

				452.47		1.310094

				452.49		1.321637

				452.51		1.327408

				452.53		1.338951

				452.55		1.344722

				452.57		1.338951

				452.59		1.338951

				452.61		1.333179

				452.64		1.333179

				452.66		1.327408

				452.68		1.327408

				452.7		1.321637

				452.72		1.321637

				452.74		1.321637

				452.76		1.321637

				452.78		1.315865

				452.8		1.315865

				452.82		1.315865

				452.85		1.310094

				452.87		1.315865

				452.89		1.310094

				452.91		1.310094

				452.93		1.310094

				452.95		1.304323

				452.97		1.304323

				452.99		1.304323

				453.01		1.298551

				453.03		1.304323

				453.06		1.304323

				453.08		1.304323

				453.1		1.304323

				453.12		1.304323

				453.14		1.310094

				453.16		1.304323

				453.18		1.304323

				453.2		1.304323

				453.22		1.298551

				453.25		1.287009

				453.27		1.269695

				453.29		1.263923

				453.31		1.258152

				453.33		1.258152

				453.35		1.258152

				453.37		1.263923

				453.39		1.258152

				453.41		1.263923

				453.43		1.258152

				453.46		1.258152

				453.48		1.258152

				453.5		1.258152

				453.52		1.263923

				453.54		1.258152

				453.56		1.258152

				453.58		1.258152

				453.6		1.263923

				453.62		1.263923

				453.64		1.263923

				453.67		1.263923

				453.69		1.263923

				453.71		1.269695

				453.73		1.263923

				453.75		1.269695

				453.77		1.263923

				453.79		1.263923

				453.81		1.263923

				453.83		1.263923

				453.85		1.263923

				453.87		1.263923

				453.9		1.263923

				453.92		1.263923

				453.94		1.258152

				453.96		1.263923

				453.98		1.263923

				454		1.258152

				454.02		1.258152

				454.04		1.258152

				454.06		1.258152

				454.08		1.258152

				454.11		1.258152

				454.13		1.258152

				454.15		1.258152

				454.17		1.258152

				454.19		1.258152

				454.21		1.258152

				454.23		1.258152

				454.25		1.258152

				454.27		1.258152

				454.29		1.258152

				454.32		1.258152

				454.34		1.258152

				454.36		1.252381

				454.38		1.252381

				454.4		1.252381

				454.42		1.252381

				454.44		1.252381

				454.46		1.252381

				454.48		1.252381

				454.5		1.252381

				454.52		1.252381

				454.55		1.252381

				454.57		1.252381

				454.59		1.252381

				454.61		1.252381

				454.63		1.252381

				454.65		1.252381

				454.67		1.252381

				454.69		1.252381

				454.71		1.252381

				454.73		1.252381

				454.76		1.252381

				454.78		1.252381

				454.8		1.252381

				454.82		1.252381

				454.84		1.252381

				454.86		1.252381

				454.88		1.252381

				454.9		1.252381

				454.92		1.252381

				454.94		1.252381

				454.97		1.252381

				454.99		1.252381

				455.01		1.252381

				455.03		1.252381

				455.05		1.252381

				455.07		1.252381

				455.09		1.252381

				455.11		1.252381

				455.13		1.252381

				455.15		1.252381

				455.17		1.252381

				455.2		1.252381

				455.22		1.252381

				455.24		1.252381

				455.26		1.252381

				455.28		1.252381

				455.3		1.252381

				455.32		1.252381

				455.34		1.252381

				455.36		1.252381

				455.38		1.252381

				455.41		1.246609

				455.43		1.252381

				455.45		1.252381

				455.47		1.252381

				455.49		1.246609

				455.51		1.246609

				455.53		1.252381

				455.55		1.252381

				455.57		1.252381

				455.59		1.252381

				455.61		1.252381

				455.64		1.252381

				455.66		1.252381

				455.68		1.252381

				455.7		1.252381

				455.72		1.252381

				455.74		1.258152

				455.76		1.252381

				455.78		1.258152

				455.8		1.258152

				455.82		1.252381

				455.85		1.258152

				455.87		1.258152

				455.89		1.258152

				455.91		1.258152

				455.93		1.258152

				455.95		1.258152

				455.97		1.258152

				455.99		1.258152

				456.01		1.258152

				456.03		1.263923

				456.06		1.263923

				456.08		1.263923

				456.1		1.263923

				456.12		1.263923

				456.14		1.263923

				456.16		1.263923

				456.18		1.263923

				456.2		1.263923

				456.22		1.263923

				456.24		1.263923

				456.26		1.263923

				456.29		1.263923

				456.31		1.263923

				456.33		1.263923

				456.35		1.263923

				456.37		1.263923

				456.39		1.263923

				456.41		1.263923

				456.43		1.263923

				456.45		1.269695

				456.47		1.269695

				456.5		1.269695

				456.52		1.269695

				456.54		1.269695

				456.56		1.269695

				456.58		1.269695

				456.6		1.269695

				456.62		1.269695

				456.64		1.269695

				456.66		1.269695

				456.68		1.269695

				456.71		1.269695

				456.73		1.269695

				456.75		1.269695

				456.77		1.269695

				456.79		1.269695

				456.81		1.269695

				456.83		1.269695

				456.85		1.269695

				456.87		1.269695

				456.89		1.269695

				456.91		1.269695

				456.94		1.269695

				456.96		1.269695

				456.98		1.269695

				457		1.269695

				457.02		1.269695

				457.04		1.269695

				457.06		1.269695

				457.08		1.269695

				457.1		1.269695

				457.12		1.269695

				457.15		1.269695

				457.17		1.275466

				457.19		1.269695

				457.21		1.269695

				457.23		1.269695

				457.25		1.269695

				457.27		1.269695

				457.29		1.269695

				457.31		1.269695

				457.33		1.269695

				457.36		1.269695

				457.38		1.269695

				457.4		1.269695

				457.42		1.269695

				457.44		1.269695

				457.46		1.269695

				457.48		1.269695

				457.5		1.269695

				457.52		1.269695

				457.54		1.269695

				457.56		1.269695

				457.59		1.269695

				457.61		1.269695

				457.63		1.269695

				457.65		1.269695

				457.67		1.269695

				457.69		1.269695

				457.71		1.269695

				457.73		1.269695

				457.75		1.269695

				457.77		1.269695

				457.8		1.269695

				457.82		1.269695

				457.84		1.269695

				457.86		1.269695

				457.88		1.269695

				457.9		1.269695

				457.92		1.269695

				457.94		1.269695

				457.96		1.269695

				457.98		1.269695

				458.01		1.269695

				458.03		1.263923

				458.05		1.263923

				458.07		1.263923

				458.09		1.263923

				458.11		1.263923

				458.13		1.263923

				458.15		1.263923

				458.17		1.263923

				458.19		1.263923

				458.22		1.263923

				458.24		1.263923

				458.26		1.263923

				458.28		1.263923

				458.3		1.263923

				458.32		1.263923

				458.34		1.263923

				458.36		1.263923

				458.38		1.263923

				458.4		1.263923

				458.42		1.263923

				458.45		1.263923

				458.47		1.263923

				458.49		1.263923

				458.51		1.263923

				458.53		1.263923

				458.55		1.263923

				458.57		1.263923

				458.59		1.263923

				458.61		1.263923

				458.63		1.263923

				458.66		1.263923

				458.68		1.263923

				458.7		1.258152

				458.72		1.263923

				458.74		1.258152

				458.76		1.258152

				458.78		1.263923

				458.8		1.258152

				458.82		1.258152

				458.84		1.258152

				458.87		1.258152

				458.89		1.258152

				458.91		1.258152

				458.93		1.263923

				458.95		1.263923

				458.97		1.263923

				458.99		1.263923

				459.01		1.263923

				459.03		1.263923

				459.05		1.263923

				459.07		1.263923

				459.1		1.263923

				459.12		1.263923

				459.14		1.263923

				459.16		1.263923

				459.18		1.263923

				459.2		1.263923

				459.22		1.263923

				459.24		1.263923

				459.26		1.263923

				459.28		1.263923

				459.31		1.263923

				459.33		1.263923

				459.35		1.263923

				459.37		1.263923

				459.39		1.263923

				459.41		1.263923

				459.43		1.263923

				459.45		1.263923

				459.47		1.263923

				459.49		1.263923

				459.52		1.263923

				459.54		1.263923

				459.56		1.263923

				459.58		1.263923

				459.6		1.263923

				459.62		1.263923

				459.64		1.263923

				459.66		1.263923

				459.68		1.263923

				459.7		1.263923

				459.72		1.263923

				459.75		1.263923

				459.77		1.263923

				459.79		1.263923

				459.81		1.263923

				459.83		1.263923

				459.85		1.258152

				459.87		1.258152

				459.89		1.258152

				459.91		1.258152

				459.93		1.263923

				459.96		1.258152

				459.98		1.263923

				460		1.263923

				460.02		1.263923

				460.04		1.263923

				460.06		1.263923

				460.08		1.263923

				460.1		1.263923

				460.12		1.263923

				460.14		1.263923

				460.17		1.263923

				460.19		1.263923

				460.21		1.263923

				460.23		1.263923

				460.25		1.263923

				460.27		1.263923

				460.29		1.263923

				460.31		1.263923

				460.33		1.263923

				460.35		1.263923

				460.38		1.263923

				460.4		1.263923

				460.42		1.258152

				460.44		1.263923

				460.46		1.263923

				460.48		1.263923

				460.5		1.263923

				460.52		1.263923

				460.54		1.263923

				460.56		1.263923

				460.58		1.263923

				460.61		1.263923

				460.63		1.263923

				460.65		1.263923

				460.67		1.258152

				460.69		1.258152

				460.71		1.263923

				460.73		1.263923

				460.75		1.258152

				460.77		1.263923

				460.79		1.258152

				460.82		1.258152

				460.84		1.258152

				460.86		1.258152

				460.88		1.263923

				460.9		1.258152

				460.92		1.258152

				460.94		1.263923

				460.96		1.263923

				460.98		1.263923

				461		1.258152

				461.03		1.263923

				461.05		1.263923

				461.07		1.263923

				461.09		1.263923

				461.11		1.258152

				461.13		1.258152

				461.15		1.263923

				461.17		1.263923

				461.19		1.263923

				461.21		1.263923

				461.23		1.263923

				461.26		1.263923

				461.28		1.263923

				461.3		1.263923

				461.32		1.263923

				461.34		1.263923

				461.36		1.263923

				461.38		1.263923

				461.4		1.263923

				461.42		1.263923

				461.44		1.263923

				461.46		1.263923

				461.49		1.263923

				461.51		1.263923

				461.53		1.269695

				461.55		1.263923

				461.57		1.263923

				461.59		1.263923

				461.61		1.263923

				461.63		1.263923

				461.65		1.263923

				461.67		1.263923

				461.7		1.263923

				461.72		1.263923

				461.74		1.263923

				461.76		1.263923

				461.78		1.269695

				461.8		1.269695

				461.82		1.269695

				461.84		1.269695

				461.86		1.269695

				461.88		1.269695

				461.9		1.269695

				461.93		1.269695

				461.95		1.269695

				461.97		1.269695

				461.99		1.269695

				462.01		1.269695

				462.03		1.269695

				462.05		1.269695

				462.07		1.269695

				462.09		1.269695

				462.11		1.269695

				462.14		1.269695

				462.16		1.269695

				462.18		1.269695

				462.2		1.269695

				462.22		1.269695

				462.24		1.275466

				462.26		1.269695

				462.28		1.275466

				462.3		1.275466

				462.32		1.275466

				462.35		1.275466

				462.37		1.275466

				462.39		1.275466

				462.41		1.275466

				462.43		1.275466

				462.45		1.275466

				462.47		1.275466

				462.49		1.275466

				462.51		1.275466

				462.53		1.275466

				462.55		1.275466

				462.58		1.275466

				462.6		1.275466

				462.62		1.275466

				462.64		1.275466

				462.66		1.275466

				462.68		1.275466

				462.7		1.275466

				462.72		1.275466

				462.74		1.275466

				462.76		1.281237

				462.79		1.281237

				462.81		1.281237

				462.83		1.281237

				462.85		1.281237

				462.87		1.281237

				462.89		1.281237

				462.91		1.281237

				462.93		1.281237

				462.95		1.281237

				462.97		1.281237

				463		1.281237

				463.02		1.281237

				463.04		1.281237

				463.06		1.281237

				463.08		1.281237

				463.1		1.281237

				463.12		1.281237

				463.14		1.281237

				463.16		1.281237

				463.18		1.281237

				463.2		1.275466

				463.23		1.281237

				463.25		1.275466

				463.27		1.275466

				463.29		1.275466

				463.31		1.275466

				463.33		1.275466

				463.35		1.275466

				463.37		1.275466

				463.39		1.275466

				463.41		1.275466

				463.44		1.275466

				463.46		1.269695

				463.48		1.275466

				463.5		1.269695

				463.52		1.269695

				463.54		1.269695

				463.56		1.269695

				463.58		1.269695

				463.6		1.269695

				463.62		1.269695

				463.64		1.269695

				463.67		1.269695

				463.69		1.269695

				463.71		1.269695

				463.73		1.269695

				463.75		1.269695

				463.77		1.269695

				463.79		1.269695

				463.81		1.269695

				463.83		1.269695

				463.85		1.269695

				463.88		1.269695

				463.9		1.269695

				463.92		1.269695

				463.94		1.269695

				463.96		1.269695

				463.98		1.269695

				464		1.269695

				464.02		1.269695

				464.04		1.269695

				464.06		1.269695

				464.08		1.269695

				464.11		1.269695

				464.13		1.269695

				464.15		1.269695

				464.17		1.269695

				464.19		1.269695

				464.21		1.269695

				464.23		1.269695

				464.25		1.269695

				464.27		1.269695

				464.29		1.269695

				464.31		1.263923

				464.34		1.263923

				464.36		1.263923

				464.38		1.263923

				464.4		1.263923

				464.42		1.263923

				464.44		1.263923

				464.46		1.263923

				464.48		1.263923

				464.5		1.263923

				464.52		1.263923

				464.55		1.263923

				464.57		1.263923

				464.59		1.263923

				464.61		1.263923

				464.63		1.263923

				464.65		1.263923

				464.67		1.263923

				464.69		1.263923

				464.71		1.263923

				464.73		1.263923

				464.76		1.263923

				464.78		1.263923

				464.8		1.263923

				464.82		1.263923

				464.84		1.263923

				464.86		1.258152

				464.88		1.258152

				464.9		1.258152

				464.92		1.258152

				464.94		1.258152

				464.96		1.258152

				464.99		1.258152

				465.01		1.258152

				465.03		1.258152

				465.05		1.258152

				465.07		1.258152

				465.09		1.258152

				465.11		1.258152

				465.13		1.258152

				465.15		1.258152

				465.17		1.258152

				465.2		1.258152

				465.22		1.258152

				465.24		1.258152

				465.26		1.258152

				465.28		1.258152

				465.3		1.258152

				465.32		1.258152

				465.34		1.258152

				465.36		1.258152

				465.38		1.263923

				465.41		1.263923

				465.43		1.263923

				465.45		1.263923

				465.47		1.263923

				465.49		1.263923

				465.51		1.263923

				465.53		1.263923

				465.55		1.263923

				465.57		1.263923

				465.59		1.263923

				465.62		1.263923

				465.64		1.263923

				465.66		1.263923

				465.68		1.263923

				465.7		1.263923

				465.72		1.263923

				465.74		1.263923

				465.76		1.263923

				465.78		1.263923

				465.8		1.263923

				465.83		1.263923

				465.85		1.263923

				465.87		1.269695

				465.89		1.269695

				465.91		1.269695

				465.93		1.269695

				465.95		1.269695

				465.97		1.269695

				465.99		1.269695

				466.01		1.269695

				466.04		1.269695

				466.06		1.269695

				466.08		1.269695

				466.1		1.269695

				466.12		1.269695

				466.14		1.269695

				466.16		1.269695

				466.18		1.269695

				466.2		1.269695

				466.22		1.269695

				466.25		1.269695

				466.27		1.269695

				466.29		1.269695

				466.31		1.269695

				466.33		1.269695

				466.35		1.269695

				466.37		1.275466

				466.39		1.275466

				466.41		1.275466

				466.43		1.275466

				466.46		1.275466

				466.48		1.275466

				466.5		1.275466

				466.52		1.275466

				466.54		1.275466

				466.56		1.275466

				466.58		1.275466

				466.6		1.275466

				466.62		1.275466

				466.64		1.275466

				466.66		1.281237

				466.69		1.281237

				466.71		1.281237

				466.73		1.281237

				466.75		1.281237

				466.77		1.281237

				466.79		1.281237

				466.81		1.281237

				466.83		1.281237

				466.85		1.281237

				466.88		1.281237

				466.9		1.281237

				466.92		1.281237

				466.94		1.281237

				466.96		1.281237

				466.98		1.281237

				467		1.281237

				467.02		1.281237

				467.04		1.281237

				467.06		1.281237

				467.08		1.281237

				467.11		1.281237

				467.13		1.281237

				467.15		1.281237

				467.17		1.281237

				467.19		1.287009

				467.21		1.281237

				467.23		1.281237

				467.25		1.287009

				467.27		1.281237

				467.29		1.281237

				467.32		1.281237

				467.34		1.281237

				467.36		1.281237

				467.38		1.281237

				467.4		1.287009

				467.42		1.281237

				467.44		1.281237

				467.46		1.281237

				467.48		1.287009

				467.5		1.281237

				467.53		1.281237

				467.55		1.287009

				467.57		1.287009

				467.59		1.287009

				467.61		1.287009

				467.63		1.287009

				467.65		1.287009

				467.67		1.287009

				467.69		1.287009

				467.71		1.287009

				467.74		1.287009

				467.76		1.287009

				467.78		1.287009

				467.8		1.287009

				467.82		1.287009

				467.84		1.287009

				467.86		1.287009

				467.88		1.287009

				467.9		1.287009

				467.92		1.287009

				467.95		1.287009

				467.97		1.287009

				467.99		1.287009

				468.01		1.281237

				468.03		1.287009

				468.05		1.287009

				468.07		1.281237

				468.09		1.287009

				468.11		1.287009

				468.13		1.287009

				468.16		1.281237

				468.18		1.287009

				468.2		1.287009

				468.22		1.287009

				468.24		1.287009

				468.26		1.287009

				468.28		1.287009

				468.3		1.287009

				468.32		1.287009

				468.34		1.287009

				468.37		1.287009

				468.39		1.287009

				468.41		1.287009

				468.43		1.287009

				468.45		1.287009

				468.47		1.287009

				468.49		1.287009

				468.51		1.287009

				468.53		1.287009

				468.55		1.287009

				468.58		1.287009

				468.6		1.281237

				468.62		1.287009

				468.64		1.287009

				468.66		1.281237

				468.68		1.281237

				468.7		1.287009

				468.72		1.287009

				468.74		1.281237

				468.76		1.287009

				468.78		1.281237

				468.81		1.281237

				468.83		1.287009

				468.85		1.287009

				468.87		1.287009

				468.89		1.287009

				468.91		1.287009

				468.93		1.287009

				468.95		1.287009

				468.97		1.287009

				468.99		1.287009

				469.02		1.287009

				469.04		1.287009

				469.06		1.287009

				469.08		1.287009

				469.1		1.281237

				469.12		1.287009

				469.14		1.287009

				469.16		1.287009

				469.18		1.287009

				469.2		1.287009

				469.22		1.287009

				469.25		1.287009

				469.27		1.287009

				469.29		1.287009

				469.31		1.287009

				469.33		1.287009

				469.35		1.287009

				469.37		1.287009

				469.39		1.287009

				469.41		1.287009

				469.43		1.287009

				469.46		1.287009

				469.48		1.287009

				469.5		1.29278

				469.52		1.287009

				469.54		1.29278

				469.56		1.29278

				469.58		1.29278

				469.6		1.29278

				469.62		1.29278

				469.64		1.29278

				469.67		1.29278

				469.69		1.29278

				469.71		1.29278

				469.73		1.29278

				469.75		1.29278

				469.77		1.29278

				469.79		1.29278

				469.81		1.29278

				469.83		1.29278

				469.85		1.29278

				469.87		1.29278

				469.9		1.29278

				469.92		1.29278

				469.94		1.29278

				469.96		1.29278

				469.98		1.29278

				470		1.29278

				470.02		1.29278

				470.04		1.29278

				470.06		1.29278

				470.08		1.298551

				470.11		1.29278

				470.13		1.29278

				470.15		1.298551

				470.17		1.298551

				470.19		1.298551

				470.21		1.29278

				470.23		1.29278

				470.25		1.298551

				470.27		1.29278

				470.29		1.29278

				470.31		1.29278

				470.34		1.29278

				470.36		1.29278

				470.38		1.29278

				470.4		1.29278

				470.42		1.29278

				470.44		1.29278

				470.46		1.29278

				470.48		1.29278

				470.5		1.29278

				470.52		1.29278

				470.55		1.29278

				470.57		1.29278

				470.59		1.29278

				470.61		1.29278

				470.63		1.29278

				470.65		1.29278

				470.67		1.29278

				470.69		1.29278

				470.71		1.29278

				470.73		1.29278

				470.75		1.29278

				470.78		1.29278

				470.8		1.29278

				470.82		1.29278

				470.84		1.29278

				470.86		1.29278

				470.88		1.29278

				470.9		1.29278

				470.92		1.29278

				470.94		1.29278

				470.96		1.29278

				470.99		1.29278

				471.01		1.29278

				471.03		1.29278

				471.05		1.29278

				471.07		1.29278

				471.09		1.29278

				471.11		1.29278

				471.13		1.29278

				471.15		1.29278

				471.17		1.29278

				471.19		1.29278

				471.22		1.29278

				471.24		1.29278

				471.26		1.29278

				471.28		1.29278

				471.3		1.29278

				471.32		1.29278

				471.34		1.287009

				471.36		1.29278

				471.38		1.287009

				471.4		1.287009

				471.43		1.287009

				471.45		1.29278

				471.47		1.287009

				471.49		1.287009

				471.51		1.29278

				471.53		1.29278

				471.55		1.287009

				471.57		1.287009

				471.59		1.29278

				471.61		1.287009

				471.64		1.29278

				471.66		1.29278

				471.68		1.29278

				471.7		1.287009

				471.72		1.287009

				471.74		1.287009

				471.76		1.287009

				471.78		1.287009

				471.8		1.287009

				471.82		1.287009

				471.85		1.287009

				471.87		1.287009

				471.89		1.287009

				471.91		1.287009

				471.93		1.287009

				471.95		1.287009

				471.97		1.287009

				471.99		1.287009

				472.01		1.287009

				472.03		1.287009

				472.05		1.287009

				472.08		1.287009

				472.1		1.287009

				472.12		1.287009

				472.14		1.287009

				472.16		1.287009

				472.18		1.287009

				472.2		1.287009

				472.22		1.287009

				472.24		1.287009

				472.26		1.281237

				472.28		1.287009

				472.31		1.287009

				472.33		1.281237

				472.35		1.287009

				472.37		1.287009

				472.39		1.287009

				472.41		1.287009

				472.43		1.287009

				472.45		1.287009

				472.47		1.287009

				472.49		1.287009

				472.52		1.287009

				472.54		1.287009

				472.56		1.287009

				472.58		1.287009

				472.6		1.287009

				472.62		1.287009

				472.64		1.287009

				472.66		1.287009

				472.68		1.287009

				472.7		1.287009

				472.72		1.287009

				472.75		1.287009

				472.77		1.287009

				472.79		1.29278

				472.81		1.29278

				472.83		1.29278

				472.85		1.29278

				472.87		1.29278

				472.89		1.29278

				472.91		1.29278

				472.93		1.29278

				472.96		1.29278

				472.98		1.29278

				473		1.29278

				473.02		1.29278

				473.04		1.29278

				473.06		1.29278

				473.08		1.29278

				473.1		1.29278

				473.12		1.29278

				473.14		1.29278

				473.17		1.29278

				473.19		1.29278

				473.21		1.29278

				473.23		1.29278

				473.25		1.29278

				473.27		1.29278

				473.29		1.29278

				473.31		1.29278

				473.33		1.298551

				473.35		1.298551

				473.37		1.298551

				473.4		1.298551

				473.42		1.298551

				473.44		1.298551

				473.46		1.298551

				473.48		1.298551

				473.5		1.298551

				473.52		1.298551

				473.54		1.298551

				473.56		1.298551

				473.58		1.298551

				473.61		1.298551

				473.63		1.298551

				473.65		1.298551

				473.67		1.298551

				473.69		1.298551

				473.71		1.298551

				473.73		1.298551

				473.75		1.298551

				473.77		1.298551

				473.79		1.298551

				473.81		1.298551

				473.84		1.304323

				473.86		1.304323

				473.88		1.304323

				473.9		1.304323

				473.92		1.304323

				473.94		1.304323

				473.96		1.304323

				473.98		1.304323

				474		1.304323

				474.02		1.304323

				474.04		1.304323

				474.07		1.304323

				474.09		1.304323

				474.11		1.304323

				474.13		1.304323

				474.15		1.304323

				474.17		1.304323

				474.19		1.304323

				474.21		1.310094

				474.23		1.310094

				474.25		1.310094

				474.28		1.310094

				474.3		1.310094

				474.32		1.310094

				474.34		1.310094

				474.36		1.310094

				474.38		1.310094

				474.4		1.310094

				474.42		1.310094

				474.44		1.310094

				474.46		1.310094

				474.49		1.310094

				474.51		1.310094

				474.53		1.310094

				474.55		1.310094

				474.57		1.310094

				474.59		1.310094

				474.61		1.310094

				474.63		1.310094

				474.65		1.310094

				474.67		1.310094

				474.7		1.310094

				474.72		1.315865

				474.74		1.310094

				474.76		1.310094

				474.78		1.310094

				474.8		1.315865

				474.82		1.310094

				474.84		1.315865

				474.86		1.310094

				474.88		1.315865

				474.91		1.310094

				474.93		1.310094

				474.95		1.310094

				474.97		1.310094

				474.99		1.310094

				475.01		1.310094

				475.03		1.310094

				475.05		1.310094

				475.07		1.310094

				475.09		1.310094

				475.12		1.310094

				475.14		1.310094

				475.16		1.310094

				475.18		1.310094

				475.2		1.310094

				475.22		1.310094

				475.24		1.310094

				475.26		1.310094

				475.28		1.310094

				475.3		1.310094

				475.32		1.310094

				475.35		1.310094

				475.37		1.310094

				475.39		1.310094

				475.41		1.310094

				475.43		1.310094

				475.45		1.310094

				475.47		1.310094

				475.49		1.310094

				475.51		1.310094

				475.53		1.310094

				475.56		1.310094

				475.58		1.310094

				475.6		1.310094

				475.62		1.310094

				475.64		1.310094

				475.66		1.310094

				475.68		1.310094

				475.7		1.310094

				475.72		1.315865

				475.74		1.315865

				475.76		1.310094

				475.79		1.315865

				475.81		1.310094

				475.83		1.310094

				475.85		1.310094

				475.87		1.315865

				475.89		1.310094

				475.91		1.310094

				475.93		1.310094

				475.95		1.310094

				475.97		1.310094

				476		1.310094

				476.02		1.310094

				476.04		1.310094

				476.06		1.310094

				476.08		1.310094

				476.1		1.310094

				476.12		1.310094

				476.14		1.310094

				476.16		1.310094

				476.18		1.310094

				476.21		1.310094

				476.23		1.310094

				476.25		1.304323

				476.27		1.310094

				476.29		1.304323

				476.31		1.304323

				476.33		1.304323

				476.35		1.304323

				476.37		1.304323

				476.39		1.304323

				476.41		1.304323

				476.44		1.304323

				476.46		1.304323

				476.48		1.304323

				476.5		1.304323

				476.52		1.304323

				476.54		1.304323

				476.56		1.304323

				476.58		1.304323

				476.6		1.298551

				476.62		1.304323

				476.65		1.304323

				476.67		1.304323

				476.69		1.298551

				476.71		1.304323

				476.73		1.304323

				476.75		1.304323

				476.77		1.298551

				476.79		1.304323

				476.81		1.298551

				476.83		1.298551

				476.85		1.298551

				476.88		1.298551

				476.9		1.298551

				476.92		1.298551

				476.94		1.304323

				476.96		1.298551

				476.98		1.298551

				477		1.298551

				477.02		1.298551

				477.04		1.298551

				477.06		1.298551

				477.09		1.298551

				477.11		1.298551

				477.13		1.298551

				477.15		1.298551

				477.17		1.298551

				477.19		1.298551

				477.21		1.298551

				477.23		1.298551

				477.25		1.298551

				477.27		1.298551

				477.29		1.298551

				477.32		1.298551

				477.34		1.298551

				477.36		1.298551

				477.38		1.298551

				477.4		1.298551

				477.42		1.298551

				477.44		1.298551

				477.46		1.298551

				477.48		1.298551

				477.5		1.298551

				477.53		1.298551

				477.55		1.298551

				477.57		1.298551

				477.59		1.298551

				477.61		1.298551

				477.63		1.298551

				477.65		1.298551

				477.67		1.298551

				477.69		1.298551

				477.71		1.298551

				477.74		1.298551

				477.76		1.298551

				477.78		1.298551

				477.8		1.298551

				477.82		1.298551

				477.84		1.298551

				477.86		1.298551

				477.88		1.298551

				477.9		1.298551

				477.92		1.298551

				477.94		1.29278

				477.97		1.29278

				477.99		1.298551

				478.01		1.298551

				478.03		1.298551

				478.05		1.298551

				478.07		1.298551

				478.09		1.298551

				478.11		1.298551

				478.13		1.298551

				478.15		1.298551

				478.18		1.298551

				478.2		1.298551

				478.22		1.298551

				478.24		1.298551

				478.26		1.298551

				478.28		1.298551

				478.3		1.298551

				478.32		1.298551

				478.34		1.298551

				478.36		1.298551

				478.39		1.298551

				478.41		1.298551

				478.43		1.304323

				478.45		1.304323

				478.47		1.304323

				478.49		1.304323

				478.51		1.304323

				478.53		1.304323

				478.55		1.304323

				478.57		1.304323

				478.59		1.304323

				478.62		1.304323

				478.64		1.304323

				478.66		1.304323

				478.68		1.304323

				478.7		1.304323

				478.72		1.304323

				478.74		1.304323

				478.76		1.304323

				478.78		1.304323

				478.8		1.304323

				478.83		1.304323

				478.85		1.310094

				478.87		1.310094

				478.89		1.310094

				478.91		1.310094

				478.93		1.310094

				478.95		1.310094

				478.97		1.310094

				478.99		1.310094

				479.01		1.310094

				479.04		1.310094

				479.06		1.310094

				479.08		1.310094

				479.1		1.315865

				479.12		1.315865

				479.14		1.315865

				479.16		1.315865

				479.18		1.315865

				479.2		1.315865

				479.22		1.315865

				479.25		1.315865

				479.27		1.315865

				479.29		1.315865

				479.31		1.315865

				479.33		1.315865

				479.35		1.315865

				479.37		1.315865

				479.39		1.315865

				479.41		1.315865

				479.43		1.315865

				479.46		1.321637

				479.48		1.321637

				479.5		1.321637

				479.52		1.321637

				479.54		1.315865

				479.56		1.321637

				479.58		1.321637

				479.6		1.321637

				479.62		1.315865

				479.64		1.321637

				479.67		1.321637

				479.69		1.321637

				479.71		1.321637

				479.73		1.321637

				479.75		1.321637

				479.77		1.321637

				479.79		1.321637

				479.81		1.321637

				479.83		1.321637

				479.85		1.321637

				479.88		1.321637

				479.9		1.321637

				479.92		1.321637

				479.94		1.321637

				479.96		1.321637

				479.98		1.327408

				480		1.327408

				480.02		1.327408

				480.04		1.327408

				480.06		1.327408

				480.08		1.327408

				480.11		1.327408

				480.13		1.327408

				480.15		1.327408

				480.17		1.327408

				480.19		1.327408

				480.21		1.327408

				480.23		1.327408

				480.25		1.327408

				480.27		1.327408

				480.29		1.327408

				480.32		1.327408

				480.34		1.327408

				480.36		1.327408

				480.38		1.327408

				480.4		1.327408

				480.42		1.327408

				480.44		1.327408

				480.46		1.327408

				480.48		1.327408

				480.5		1.327408

				480.53		1.327408

				480.55		1.327408

				480.57		1.327408

				480.59		1.327408

				480.61		1.327408

				480.63		1.327408

				480.65		1.327408

				480.67		1.327408

				480.69		1.327408

				480.71		1.327408

				480.74		1.327408

				480.76		1.327408

				480.78		1.327408

				480.8		1.327408

				480.82		1.327408

				480.84		1.327408

				480.86		1.327408

				480.88		1.327408

				480.9		1.327408

				480.92		1.327408

				480.95		1.327408

				480.97		1.327408

				480.99		1.327408

				481.01		1.327408

				481.03		1.327408

				481.05		1.327408

				481.07		1.327408

				481.09		1.327408

				481.11		1.327408

				481.13		1.327408

				481.16		1.327408

				481.18		1.327408

				481.2		1.327408

				481.22		1.327408

				481.24		1.327408

				481.26		1.327408

				481.28		1.327408

				481.3		1.327408

				481.32		1.327408

				481.34		1.321637

				481.37		1.327408

				481.39		1.327408

				481.41		1.327408

				481.43		1.327408

				481.45		1.327408

				481.47		1.327408

				481.49		1.327408

				481.51		1.327408

				481.53		1.327408

				481.55		1.327408

				481.57		1.327408

				481.6		1.327408

				481.62		1.327408

				481.64		1.327408

				481.66		1.327408

				481.68		1.327408

				481.7		1.333179

				481.72		1.327408

				481.74		1.333179

				481.76		1.327408

				481.78		1.333179

				481.81		1.333179

				481.83		1.327408

				481.85		1.333179

				481.87		1.333179

				481.89		1.333179

				481.91		1.333179

				481.93		1.333179

				481.95		1.333179

				481.97		1.333179

				481.99		1.333179

				482.02		1.327408

				482.04		1.327408

				482.06		1.327408

				482.08		1.327408

				482.1		1.327408

				482.12		1.327408

				482.14		1.327408

				482.16		1.327408

				482.18		1.333179

				482.2		1.327408

				482.23		1.327408

				482.25		1.327408

				482.27		1.327408

				482.29		1.327408

				482.31		1.327408

				482.33		1.327408

				482.35		1.327408

				482.37		1.327408

				482.39		1.327408

				482.42		1.327408

				482.44		1.327408

				482.46		1.327408

				482.48		1.327408

				482.5		1.327408

				482.52		1.327408

				482.54		1.327408

				482.56		1.327408

				482.58		1.327408

				482.6		1.327408

				482.63		1.327408

				482.65		1.327408

				482.67		1.327408

				482.69		1.327408

				482.71		1.327408

				482.73		1.327408

				482.75		1.327408

				482.77		1.327408

				482.79		1.327408

				482.81		1.327408

				482.84		1.327408

				482.86		1.327408

				482.88		1.333179

				482.9		1.333179

				482.92		1.333179

				482.94		1.333179

				482.96		1.333179

				482.98		1.333179

				483		1.333179

				483.02		1.333179

				483.05		1.333179

				483.07		1.333179

				483.09		1.333179

				483.11		1.333179

				483.13		1.333179

				483.15		1.333179

				483.17		1.333179

				483.19		1.333179

				483.21		1.333179

				483.23		1.333179

				483.26		1.333179

				483.28		1.333179

				483.3		1.333179

				483.32		1.333179

				483.34		1.333179

				483.36		1.333179

				483.38		1.338951

				483.4		1.338951

				483.42		1.338951

				483.44		1.338951

				483.47		1.338951

				483.49		1.338951

				483.51		1.338951

				483.53		1.333179

				483.55		1.338951

				483.57		1.338951

				483.59		1.333179

				483.61		1.333179

				483.63		1.333179

				483.65		1.333179

				483.68		1.333179

				483.7		1.333179

				483.72		1.333179

				483.74		1.333179

				483.76		1.333179

				483.78		1.333179

				483.8		1.333179

				483.82		1.333179

				483.84		1.338951

				483.86		1.333179

				483.89		1.333179

				483.91		1.333179

				483.93		1.333179

				483.95		1.333179

				483.97		1.333179

				483.99		1.333179

				484.01		1.333179

				484.03		1.333179

				484.05		1.333179

				484.08		1.333179

				484.1		1.338951

				484.12		1.338951

				484.14		1.338951

				484.16		1.333179

				484.18		1.333179

				484.2		1.338951

				484.22		1.333179

				484.24		1.333179

				484.26		1.333179

				484.29		1.333179

				484.31		1.333179

				484.33		1.333179

				484.35		1.333179

				484.37		1.333179

				484.39		1.333179

				484.41		1.333179

				484.43		1.338951

				484.45		1.338951

				484.47		1.338951

				484.5		1.338951

				484.52		1.338951

				484.54		1.338951

				484.56		1.338951

				484.58		1.338951

				484.6		1.338951

				484.62		1.338951

				484.64		1.338951

				484.66		1.338951

				484.68		1.338951

				484.71		1.338951

				484.73		1.338951

				484.75		1.344722

				484.77		1.344722

				484.79		1.344722

				484.81		1.344722

				484.83		1.344722

				484.85		1.344722

				484.87		1.344722

				484.9		1.344722

				484.92		1.344722

				484.94		1.344722

				484.96		1.344722

				484.98		1.344722

				485		1.344722

				485.02		1.344722

				485.04		1.344722

				485.06		1.344722

				485.08		1.344722

				485.11		1.350493

				485.13		1.350493

				485.15		1.350493

				485.17		1.350493

				485.19		1.350493

				485.21		1.350493

				485.23		1.350493

				485.25		1.350493

				485.27		1.350493

				485.29		1.350493

				485.32		1.350493

				485.34		1.350493

				485.36		1.350493

				485.38		1.350493

				485.4		1.350493

				485.42		1.350493

				485.44		1.350493

				485.46		1.350493

				485.48		1.350493

				485.51		1.350493

				485.53		1.350493

				485.55		1.350493

				485.57		1.350493

				485.59		1.350493

				485.61		1.350493

				485.63		1.350493

				485.65		1.350493

				485.67		1.350493

				485.69		1.350493

				485.72		1.350493

				485.74		1.350493

				485.76		1.350493

				485.78		1.350493

				485.8		1.350493

				485.82		1.350493

				485.84		1.350493

				485.86		1.350493

				485.88		1.350493

				485.9		1.350493

				485.93		1.350493

				485.95		1.350493

				485.97		1.350493

				485.99		1.356265

				486.01		1.356265

				486.03		1.356265

				486.05		1.356265

				486.07		1.356265

				486.09		1.356265

				486.12		1.356265

				486.14		1.356265

				486.16		1.356265

				486.18		1.356265

				486.2		1.356265

				486.22		1.356265

				486.24		1.356265

				486.26		1.356265

				486.28		1.356265

				486.3		1.356265

				486.33		1.356265

				486.35		1.356265

				486.37		1.356265

				486.39		1.362036

				486.41		1.362036

				486.43		1.362036

				486.45		1.362036

				486.47		1.362036

				486.49		1.362036

				486.52		1.362036

				486.54		1.362036

				486.56		1.362036

				486.58		1.362036

				486.6		1.362036

				486.62		1.362036

				486.64		1.362036

				486.66		1.362036

				486.68		1.362036

				486.7		1.362036

				486.73		1.362036

				486.75		1.356265

				486.77		1.356265

				486.79		1.356265

				486.81		1.356265

				486.83		1.356265

				486.85		1.356265

				486.87		1.356265

				486.89		1.356265

				486.92		1.356265

				486.94		1.356265

				486.96		1.356265

				486.98		1.356265

				487		1.356265

				487.02		1.356265

				487.04		1.356265

				487.06		1.356265

				487.08		1.356265

				487.1		1.356265

				487.13		1.356265

				487.15		1.356265

				487.17		1.356265

				487.19		1.356265

				487.21		1.356265

				487.23		1.356265

				487.25		1.350493

				487.27		1.356265

				487.29		1.350493

				487.32		1.356265

				487.34		1.350493

				487.36		1.350493

				487.38		1.350493

				487.4		1.350493

				487.42		1.350493

				487.44		1.350493

				487.46		1.350493

				487.48		1.350493

				487.5		1.350493

				487.53		1.350493

				487.55		1.350493

				487.57		1.350493

				487.59		1.350493

				487.61		1.350493

				487.63		1.350493

				487.65		1.350493

				487.67		1.350493

				487.69		1.350493

				487.72		1.350493

				487.74		1.350493

				487.76		1.350493

				487.78		1.350493

				487.8		1.350493

				487.82		1.350493

				487.84		1.350493

				487.86		1.350493

				487.88		1.350493

				487.9		1.350493

				487.93		1.350493

				487.95		1.350493

				487.97		1.350493

				487.99		1.350493

				488.01		1.350493

				488.03		1.350493

				488.05		1.350493

				488.07		1.350493

				488.09		1.344722

				488.11		1.344722

				488.13		1.344722

				488.16		1.344722

				488.18		1.344722

				488.2		1.344722

				488.22		1.344722

				488.24		1.344722

				488.26		1.344722

				488.28		1.344722

				488.3		1.344722

				488.32		1.344722

				488.34		1.344722

				488.37		1.344722

				488.39		1.344722

				488.41		1.344722

				488.43		1.344722

				488.45		1.344722

				488.47		1.338951

				488.49		1.344722

				488.51		1.338951

				488.53		1.338951

				488.55		1.338951

				488.58		1.338951

				488.6		1.338951

				488.62		1.338951

				488.64		1.338951

				488.66		1.338951

				488.68		1.338951

				488.7		1.338951

				488.72		1.338951

				488.74		1.338951

				488.76		1.338951

				488.79		1.338951

				488.81		1.338951

				488.83		1.338951

				488.85		1.338951

				488.87		1.338951

				488.89		1.338951

				488.91		1.338951

				488.93		1.338951

				488.95		1.333179

				488.97		1.333179

				488.99		1.333179

				489.02		1.333179

				489.04		1.333179

				489.06		1.333179

				489.08		1.333179

				489.1		1.333179

				489.12		1.333179

				489.14		1.333179

				489.16		1.333179

				489.18		1.333179

				489.2		1.333179

				489.23		1.338951

				489.25		1.338951

				489.27		1.338951

				489.29		1.338951

				489.31		1.338951

				489.33		1.338951

				489.35		1.338951

				489.37		1.338951

				489.39		1.338951

				489.41		1.338951

				489.44		1.338951

				489.46		1.338951

				489.48		1.338951

				489.5		1.338951

				489.52		1.338951

				489.54		1.338951

				489.56		1.338951

				489.58		1.338951

				489.6		1.338951

				489.62		1.338951

				489.64		1.333179

				489.67		1.338951

				489.69		1.333179

				489.71		1.338951

				489.73		1.338951

				489.75		1.338951

				489.77		1.333179

				489.79		1.333179

				489.81		1.338951

				489.83		1.333179

				489.85		1.338951

				489.88		1.338951

				489.9		1.338951

				489.92		1.338951

				489.94		1.338951

				489.96		1.338951

				489.98		1.338951

				490		1.338951

				490.02		1.338951

				490.04		1.338951

				490.06		1.338951

				490.09		1.338951

				490.11		1.338951

				490.13		1.338951

				490.15		1.338951

				490.17		1.338951

				490.19		1.338951

				490.21		1.338951

				490.23		1.338951

				490.25		1.338951

				490.27		1.338951

				490.29		1.338951

				490.32		1.338951

				490.34		1.338951

				490.36		1.338951

				490.38		1.338951

				490.4		1.338951

				490.42		1.338951

				490.44		1.338951

				490.46		1.338951

				490.48		1.338951

				490.5		1.338951

				490.53		1.338951

				490.55		1.338951

				490.57		1.338951

				490.59		1.338951

				490.61		1.338951

				490.63		1.338951

				490.65		1.338951

				490.67		1.338951

				490.69		1.338951

				490.71		1.338951

				490.74		1.338951

				490.76		1.338951

				490.78		1.338951

				490.8		1.338951

				490.82		1.338951

				490.84		1.338951

				490.86		1.338951

				490.88		1.338951

				490.9		1.338951

				490.92		1.338951

				490.94		1.338951

				490.97		1.338951

				490.99		1.338951

				491.01		1.338951

				491.03		1.338951

				491.05		1.338951

				491.07		1.338951

				491.09		1.338951

				491.11		1.338951

				491.13		1.338951

				491.15		1.338951

				491.18		1.338951

				491.2		1.338951

				491.22		1.338951

				491.24		1.338951

				491.26		1.338951

				491.28		1.338951

				491.3		1.338951

				491.32		1.333179

				491.34		1.333179

				491.36		1.338951

				491.38		1.333179

				491.41		1.333179

				491.43		1.333179

				491.45		1.338951

				491.47		1.333179

				491.49		1.338951

				491.51		1.338951

				491.53		1.338951

				491.55		1.338951

				491.57		1.338951

				491.59		1.338951

				491.62		1.338951

				491.64		1.338951

				491.66		1.338951

				491.68		1.338951

				491.7		1.338951

				491.72		1.338951

				491.74		1.338951

				491.76		1.338951

				491.78		1.338951

				491.8		1.338951

				491.83		1.338951

				491.85		1.338951

				491.87		1.338951

				491.89		1.338951

				491.91		1.338951

				491.93		1.338951

				491.95		1.338951

				491.97		1.338951

				491.99		1.338951

				492.01		1.338951

				492.03		1.338951

				492.06		1.338951

				492.08		1.338951

				492.1		1.338951

				492.12		1.338951

				492.14		1.338951

				492.16		1.338951

				492.18		1.338951

				492.2		1.338951

				492.22		1.338951

				492.24		1.338951

				492.27		1.338951

				492.29		1.338951

				492.31		1.338951

				492.33		1.338951

				492.35		1.338951

				492.37		1.338951

				492.39		1.338951

		Results:

		Onset		X1		166.1		°C

				Y1		97.409		%

				X2		247.8		°C

				Y2		17.26		%

				Onset X		229.79		°C

				Onset Y		83.755		%
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RT54-0.75 GNP-0.25  MWCNT.txt


RT54-0.75 GNP-0.25 MWCNT.txt
# Name: RT54-0.75 GNP-0.25 MWCNT

# Date: Tue May 21 15:41:10 2024

# Weight: 10.8 mg

Time(s)	Temperature(°C)	Heat flow(mW)	Gas 1(sccm/min)	DSC_RAW(µV)	POWER(%)	TEMP_CJR_FURNACE(K)	TEMP_CJR_SAMPLE(K)	TEMP_FURNACE(K)	TEMP_NOM_FURNACE(K)	TEMP_NOM_SAMPLE(K)	VOLTAGE_REFERENCE(V)	VOLTAGE_SAMPLE(V)

0	29.95	0.653598	19.9998	0.000889563	0.0734039	293.15	293.15	0	303.267	303.267	0.0685617	0.0685219

1	29.97	1.82147	19.9914	0.00247905	0.128298	293.15	293.15	0	303.43	303.43	0.0685682	0.0685274

2	30.05	2.5202	20.0008	0.00342995	0.16935	293.15	293.15	0	303.588	303.588	0.0685856	0.0685465

3	30.17	2.48978	20.0008	0.00338842	0.199849	293.15	293.15	0	303.753	303.753	0.0686127	0.0685752

4	30.32	1.81934	19.9904	0.00247589	0.221112	293.15	293.15	0	303.925	303.925	0.0686458	0.0686102

5	30.49	0.76821	20.0008	0.00104538	0.239529	293.15	293.15	0	304.089	304.089	0.0686839	0.0686504

6	30.66	-0.365177	20.0008	-0.000496906	0.25313	293.15	293.15	0	304.262	304.262	0.0687218	0.0686907

7	30.85	-1.45702	20.0008	-0.00198249	0.258698	293.15	293.15	0	304.435	304.435	0.0687644	0.0687347

8	31.03	-2.47187	20.0008	-0.00336316	0.263986	293.15	293.15	0	304.599	304.599	0.068807	0.0687786

9	31.22	-3.45303	20.0008	-0.00469783	0.271492	293.15	293.15	0	304.763	304.763	0.0688516	0.0688238

10	31.42	-4.24652	20.0008	-0.00577702	0.273324	293.15	293.15	0	304.92	304.92	0.0688951	0.0688696

11	31.6	-4.82017	20.0008	-0.00655706	0.272046	293.15	293.15	0	305.091	305.091	0.0689401	0.0689142

12	31.79	-5.23865	20.0008	-0.00712592	0.275955	293.15	293.15	0	305.257	305.257	0.068984	0.0689592

13	31.97	-5.51913	20.0008	-0.00750702	0.280521	293.15	293.15	0	305.43	305.43	0.0690265	0.0690015

14	32.15	-5.69712	20.0008	-0.0077487	0.280178	293.15	293.15	0	305.602	305.602	0.0690691	0.0690443

15	32.34	-5.82554	20.0008	-0.00792291	0.278951	293.15	293.15	0	305.768	305.768	0.0691134	0.0690884

16	32.51	-5.84548	20.0008	-0.00794962	0.279893	293.15	293.15	0	305.939	305.939	0.0691553	0.0691294

17	32.69	-5.81052	20.006	-0.00790163	0.284092	293.15	293.15	0	306.098	306.098	0.0691973	0.0691717

18	32.87	-5.77895	20.0008	-0.00785829	0.286861	293.15	293.15	0	306.263	306.263	0.0692383	0.069213

19	33.05	-5.75677	20.0008	-0.00782769	0.287088	293.15	293.15	0	306.427	306.427	0.0692803	0.0692557

20	33.21	-5.69943	20.0008	-0.00774933	0.287537	293.15	293.15	0	306.586	306.586	0.0693208	0.0692952

21	33.39	-5.60743	20.0008	-0.00762384	0.289528	293.15	293.15	0	306.765	306.765	0.0693615	0.0693362

22	33.56	-5.50816	20.0008	-0.00748847	0.294927	293.15	293.15	0	306.932	306.932	0.0694023	0.0693772

23	33.73	-5.40758	20.0008	-0.00735137	0.297435	293.15	293.15	0	307.085	307.085	0.0694416	0.0694165

24	33.9	-5.30237	20.0008	-0.00720795	0.298718	293.15	293.15	0	307.261	307.261	0.069482	0.0694575

25	34.07	-5.26204	20.0008	-0.00715275	0.303924	293.15	293.15	0	307.431	307.431	0.0695222	0.0694984

26	34.24	-5.28195	20.0008	-0.00717946	0.305485	293.15	293.15	0	307.596	307.596	0.0695619	0.0695376

27	34.41	-5.27566	20.0008	-0.00717053	0.307988	293.15	293.15	0	307.754	307.754	0.0696024	0.0695776

28	34.58	-5.30043	19.9956	-0.00720383	0.311125	293.15	293.15	0	307.925	307.925	0.0696413	0.0696177

29	34.75	-5.28804	19.9904	-0.00718661	0.313021	293.15	293.15	0	308.099	308.099	0.0696811	0.0696578

30	34.91	-5.25826	19.9904	-0.00714578	0.318648	293.15	293.15	0	308.263	308.263	0.0697207	0.0696971

31	35.08	-5.24487	20.0008	-0.00712722	0.319651	293.15	293.15	0	308.436	308.436	0.0697604	0.0697363

32	35.25	-5.25791	20.0008	-0.00714457	0.321982	293.15	293.15	0	308.6	308.6	0.0698003	0.0697765

33	35.41	-5.2676	20.0008	-0.00715738	0.327371	293.15	293.15	0	308.757	308.757	0.0698389	0.069816

34	35.58	-5.31223	20.0008	-0.00721764	0.326666	293.15	293.15	0	308.928	308.928	0.06988	0.0698561

35	35.75	-5.36186	20.0008	-0.00728471	0.330079	293.15	293.15	0	309.087	309.087	0.0699199	0.0698962

36	35.92	-5.39081	20.0008	-0.00732366	0.33537	293.15	293.15	0	309.267	309.267	0.0699584	0.0699354

37	36.08	-5.37349	20.0008	-0.00729977	0.337121	293.15	293.15	0	309.417	309.417	0.0699973	0.0699746

38	36.25	-5.27681	20.0008	-0.00716806	0.338196	293.15	293.15	0	309.594	309.594	0.0700374	0.0700141

39	36.42	-5.20062	19.9956	-0.0070642	0.345335	293.15	293.15	0	309.763	309.763	0.0700764	0.0700539

40	36.59	-5.18702	20.0008	-0.00704536	0.347007	293.15	293.15	0	309.928	309.928	0.0701156	0.0700934

41	36.76	-5.22084	20.0008	-0.00709094	0.349774	293.15	293.15	0	310.084	310.084	0.0701546	0.070133

42	36.92	-5.2497	20.0008	-0.00712978	0.351107	293.15	293.15	0	310.25	310.25	0.070195	0.0701722

43	37.08	-5.25096	20.0008	-0.00713114	0.35711	293.15	293.15	0	310.421	310.421	0.0702335	0.0702107

44	37.25	-5.25029	20.0008	-0.00712985	0.360597	293.15	293.15	0	310.595	310.595	0.0702731	0.0702505

45	37.42	-5.28389	19.9956	-0.00717512	0.364691	293.15	293.15	0	310.761	310.761	0.0703125	0.07029

46	37.59	-5.25305	20.0008	-0.00713288	0.367263	293.15	293.15	0	310.933	310.933	0.0703513	0.0703296

47	37.76	-5.21626	19.9904	-0.00708255	0.372808	293.15	293.15	0	311.088	311.088	0.0703914	0.07037

48	37.93	-5.16196	19.9956	-0.00700847	0.375229	293.15	293.15	0	311.252	311.252	0.0704309	0.0704094

49	38.09	-5.14225	20.0112	-0.00698134	0.376113	293.15	293.15	0	311.426	311.426	0.0704704	0.0704491

50	38.26	-5.15486	20.0008	-0.00699811	0.378281	293.15	293.15	0	311.599	311.599	0.0705097	0.0704885

51	38.43	-5.17054	20.0008	-0.00701905	0.384555	293.15	293.15	0	311.764	311.764	0.0705489	0.0705282

52	38.6	-5.18711	20.0008	-0.00704117	0.386168	293.15	293.15	0	311.945	311.945	0.0705893	0.0705684

53	38.76	-5.1652	20.0008	-0.00701109	0.38869	293.15	293.15	0	312.093	312.093	0.0706268	0.0706056

54	38.92	-5.11529	20.0008	-0.00694299	0.394702	293.15	293.15	0	312.266	312.266	0.0706664	0.0706455

55	39.09	-5.12421	20.0008	-0.00695473	0.399952	293.15	293.15	0	312.43	312.43	0.0707055	0.070685

56	39.26	-5.11135	20.0008	-0.00693694	0.399168	293.15	293.15	0	312.593	312.593	0.0707455	0.0707244

57	39.43	-5.09093	20.0008	-0.00690886	0.404384	293.15	293.15	0	312.751	312.751	0.0707843	0.0707642

58	39.59	-5.08517	20.0008	-0.0069007	0.406501	293.15	293.15	0	312.93	312.93	0.0708233	0.0708033

59	39.76	-5.12239	19.9977	-0.00695085	0.411284	293.15	293.15	0	313.097	313.097	0.070863	0.0708431

60	39.93	-5.13364	19.9904	-0.00696576	0.415189	293.15	293.15	0	313.261	313.261	0.0709026	0.0708825

61	40.1	-5.08932	19.9977	-0.00690527	0.41835	293.15	293.15	0	313.418	313.418	0.0709413	0.0709219

62	40.26	-5.06598	20.0008	-0.00687325	0.420436	293.15	293.15	0	313.586	313.586	0.070981	0.0709615

63	40.43	-5.1515	20.0008	-0.00698893	0.42455	293.15	293.15	0	313.765	313.765	0.0710198	0.0710009

64	40.6	-5.23384	19.9987	-0.00710026	0.428592	293.15	293.15	0	313.929	313.929	0.0710596	0.0710415

65	40.76	-5.25547	19.9904	-0.00712926	0.429719	293.15	293.15	0	314.096	314.096	0.0710989	0.0710798

66	40.93	-5.28688	19.9914	-0.00717149	0.434219	293.15	293.15	0	314.269	314.269	0.0711384	0.0711199

67	41.1	-5.31093	20.0008	-0.00720375	0.437754	293.15	293.15	0	314.425	314.425	0.0711783	0.0711595

68	41.27	-5.32573	20.0008	-0.00722346	0.44157	293.15	293.15	0	314.596	314.596	0.0712172	0.0711983

69	41.44	-5.30158	20.0008	-0.00719033	0.444652	293.15	293.15	0	314.769	314.769	0.0712573	0.0712384

70	41.61	-5.28985	20.0008	-0.00717406	0.448301	293.15	293.15	0	314.926	314.926	0.0712962	0.0712783

71	41.77	-5.23356	20.0008	-0.00709736	0.450177	293.15	293.15	0	315.09	315.09	0.0713347	0.0713169

72	41.94	-5.19297	20.0008	-0.00704196	0.457053	293.15	293.15	0	315.263	315.263	0.0713736	0.0713563

73	42.1	-5.19816	20.0008	-0.00704863	0.458811	293.15	293.15	0	315.427	315.427	0.0714127	0.071396

74	42.27	-5.24149	20.0112	-0.00710702	0.46042	293.15	293.15	0	315.601	315.601	0.071453	0.0714355

75	42.44	-5.24609	19.9977	-0.00711289	0.46405	293.15	293.15	0	315.756	315.756	0.0714926	0.0714756

76	42.61	-5.22277	19.9904	-0.00708093	0.46939	293.15	293.15	0	315.93	315.93	0.0715312	0.0715142

77	42.78	-5.19895	19.9998	-0.00704825	0.469446	293.15	293.15	0	316.095	316.095	0.0715714	0.0715546

78	42.94	-5.27681	20.0008	-0.00715346	0.475173	293.15	293.15	0	316.266	316.266	0.0716098	0.0715933

79	43.11	-5.34393	20.0008	-0.00724408	0.47932	293.15	293.15	0	316.431	316.431	0.0716491	0.0716326

80	43.28	-5.34873	20.0008	-0.00725022	0.483653	293.15	293.15	0	316.598	316.598	0.0716883	0.0716723

81	43.44	-5.31365	20.0008	-0.00720232	0.485823	293.15	293.15	0	316.758	316.758	0.0717268	0.0717102

82	43.61	-5.25479	20.0008	-0.00712215	0.488005	293.15	293.15	0	316.927	316.927	0.0717669	0.0717513

83	43.78	-5.17203	20.0008	-0.00700963	0.491047	293.15	293.15	0	317.099	317.099	0.0718067	0.0717904

84	43.94	-5.10638	20.0008	-0.0069203	0.494943	293.15	293.15	0	317.259	317.259	0.0718466	0.0718297

85	44.11	-5.06102	20.0008	-0.00685848	0.499364	293.15	293.15	0	317.419	317.419	0.0718842	0.0718687

86	44.28	-5.04869	20.0008	-0.00684143	0.501939	293.15	293.15	0	317.593	317.593	0.0719236	0.0719077

87	44.45	-5.10557	20.0008	-0.00691815	0.503817	293.15	293.15	0	317.761	317.761	0.0719635	0.0719482

88	44.61	-5.20491	20.0008	-0.00705241	0.51076	293.15	293.15	0	317.93	317.93	0.072002	0.0719864

89	44.78	-5.24232	20.0008	-0.00710274	0.513194	293.15	293.15	0	318.087	318.087	0.0720412	0.0720256

90	44.94	-5.24635	20.0008	-0.00710783	0.515465	293.15	293.15	0	318.253	318.253	0.0720805	0.0720653

91	45.11	-5.21411	20.0008	-0.00706379	0.519625	293.15	293.15	0	318.425	318.425	0.07212	0.0721048

92	45.28	-5.15907	19.9998	-0.00698886	0.525034	293.15	293.15	0	318.597	318.597	0.0721595	0.0721443

93	45.44	-5.08948	19.9914	-0.00689426	0.530111	293.15	293.15	0	318.763	318.763	0.0721979	0.072183

94	45.62	-5.07305	20.0008	-0.00687164	0.530193	293.15	293.15	0	318.926	318.926	0.072238	0.0722233

95	45.78	-5.16223	20.0008	-0.00699209	0.534344	293.15	293.15	0	319.091	319.091	0.0722768	0.0722627

96	45.95	-5.2753	20.0008	-0.00714487	0.540853	293.15	293.15	0	319.264	319.264	0.0723155	0.0723017

97	46.12	-5.32036	19.9904	-0.00720552	0.543462	293.15	293.15	0	319.429	319.429	0.0723552	0.0723416

98	46.29	-5.36716	20.0008	-0.00726854	0.543968	293.15	293.15	0	319.602	319.602	0.0723948	0.0723813

99	46.46	-5.46547	20.0008	-0.00740129	0.546846	293.15	293.15	0	319.759	319.759	0.0724336	0.0724209

100	46.62	-5.52882	20.0008	-0.00748671	0.553891	293.15	293.15	0	319.929	319.929	0.0724735	0.0724603

101	46.79	-5.5133	20.0008	-0.00746532	0.555942	293.15	293.15	0	320.096	320.096	0.0725119	0.0724991

102	46.96	-5.43877	20.0008	-0.00736401	0.556146	293.15	293.15	0	320.259	320.259	0.0725523	0.0725394

103	47.12	-5.44307	20.0008	-0.00736948	0.564106	293.15	293.15	0	320.433	320.433	0.0725908	0.0725776

104	47.29	-5.45282	20.0008	-0.0073823	0.567382	293.15	293.15	0	320.595	320.595	0.0726297	0.0726174

105	47.46	-5.43024	20.0008	-0.00735135	0.570594	293.15	293.15	0	320.763	320.763	0.0726693	0.0726567

106	47.62	-5.41006	20.0008	-0.00732366	0.575184	293.15	293.15	0	320.934	320.934	0.072708	0.0726955

107	47.79	-5.37445	20.0008	-0.00727508	0.576461	293.15	293.15	0	321.084	321.084	0.0727471	0.0727353

108	47.96	-5.40319	20.0008	-0.00731361	0.578964	293.15	293.15	0	321.261	321.261	0.0727861	0.0727746

109	48.12	-5.41458	20.0029	-0.00732867	0.584963	293.15	293.15	0	321.43	321.43	0.0728258	0.0728139

110	48.29	-5.42779	20.0091	-0.00734617	0.586903	293.15	293.15	0	321.603	321.603	0.0728648	0.0728533

111	48.46	-5.46702	20.0008	-0.00739888	0.588681	293.15	293.15	0	321.751	321.751	0.0729043	0.0728929

112	48.63	-5.49162	19.9998	-0.0074318	0.59181	293.15	293.15	0	321.918	321.918	0.0729436	0.0729327

113	48.79	-5.47432	19.9904	-0.00740802	0.596362	293.15	293.15	0	322.09	322.09	0.0729824	0.0729707

114	48.96	-5.41557	20.0008	-0.00732815	0.603665	293.15	293.15	0	322.263	322.263	0.0730214	0.07301

115	49.12	-5.37708	20.0008	-0.0072757	0.607391	293.15	293.15	0	322.428	322.428	0.07306	0.0730489

116	49.29	-5.29856	20.0008	-0.00716909	0.608299	293.15	293.15	0	322.6	322.6	0.0730997	0.0730882

117	49.46	-5.1902	20.0008	-0.00702212	0.615551	293.15	293.15	0	322.764	322.764	0.0731391	0.0731276

118	49.62	-5.15901	20.0008	-0.00697957	0.618309	293.15	293.15	0	322.929	322.929	0.0731773	0.0731661

119	49.79	-5.173	20.0008	-0.00699813	0.621412	293.15	293.15	0	323.085	323.085	0.0732166	0.0732064

120	49.96	-5.24435	19.9966	-0.00709429	0.624651	293.15	293.15	0	323.259	323.259	0.0732554	0.0732454

121	50.13	-5.27637	19.9904	-0.00713726	0.630737	293.15	293.15	0	323.429	323.429	0.0732941	0.0732842

122	50.3	-5.33974	19.9998	-0.0072226	0.631254	293.15	293.15	0	323.596	323.596	0.073335	0.0733249

123	50.46	-5.38245	20.0008	-0.00728	0.636107	293.15	293.15	0	323.752	323.752	0.0733738	0.0733636

124	50.63	-5.40618	20.0008	-0.00731172	0.637201	293.15	293.15	0	323.922	323.922	0.0734133	0.0734037

125	50.8	-5.43442	20.0008	-0.00734954	0.643841	293.15	293.15	0	324.09	324.09	0.0734518	0.0734426

126	50.97	-5.46669	20.0008	-0.00739281	0.647692	293.15	293.15	0	324.263	324.263	0.0734912	0.0734818

127	51.14	-5.5083	20.0008	-0.00744869	0.649238	293.15	293.15	0	324.427	324.427	0.0735308	0.0735218

128	51.3	-5.55579	20.0008	-0.00751254	0.652593	293.15	293.15	0	324.587	324.587	0.0735692	0.0735604

129	51.47	-5.56911	20.0008	-0.00753017	0.658483	293.15	293.15	0	324.756	324.756	0.0736092	0.0735998

130	51.64	-5.58779	20.0008	-0.00755504	0.66258	293.15	293.15	0	324.925	324.925	0.0736476	0.0736395

131	51.8	-5.6067	20.0008	-0.00758022	0.665292	293.15	293.15	0	325.094	325.094	0.0736865	0.0736784

132	51.97	-5.65978	20.0008	-0.00765159	0.668449	293.15	293.15	0	325.267	325.267	0.0737259	0.0737184

133	52.14	-5.68054	20.0008	-0.00767928	0.672558	293.15	293.15	0	325.417	325.417	0.0737645	0.0737568

134	52.31	-5.67292	19.9956	-0.00766857	0.676087	293.15	293.15	0	325.588	325.588	0.0738045	0.0737973

135	52.48	-5.62582	20.0008	-0.00760452	0.680325	293.15	293.15	0	325.761	325.761	0.0738438	0.0738364

136	52.64	-5.61938	20.0008	-0.00759544	0.682301	293.15	293.15	0	325.928	325.928	0.073883	0.0738744

137	52.81	-5.72568	20.0019	-0.00773873	0.688117	293.15	293.15	0	326.098	326.098	0.0739219	0.0739138

138	52.97	-5.76982	20.0112	-0.00779798	0.694785	293.15	293.15	0	326.264	326.264	0.07396	0.0739532

139	53.14	-5.71022	20.006	-0.00771704	0.696125	293.15	293.15	0	326.419	326.419	0.0739998	0.0739927

140	53.31	-5.65646	20.0008	-0.00764399	0.698252	293.15	293.15	0	326.592	326.592	0.0740392	0.0740322

141	53.48	-5.67929	20.0008	-0.00767447	0.699237	293.15	293.15	0	326.757	326.757	0.0740787	0.0740713

142	53.65	-5.70513	20.0008	-0.00770897	0.704303	293.15	293.15	0	326.93	326.93	0.0741186	0.0741115

143	53.81	-5.6745	20.0008	-0.00766722	0.709556	293.15	293.15	0	327.094	327.094	0.0741561	0.074149

144	53.97	-5.61642	20.0008	-0.00758835	0.712658	293.15	293.15	0	327.267	327.267	0.0741951	0.0741883

145	54.14	-5.57862	20.0008	-0.0075369	0.717108	293.15	293.15	0	327.424	327.424	0.074234	0.0742275

146	54.31	-5.56727	20.0008	-0.00752119	0.722409	293.15	293.15	0	327.598	327.598	0.0742726	0.0742665

147	54.47	-5.56291	20.0008	-0.00751492	0.725685	293.15	293.15	0	327.761	327.761	0.0743119	0.0743056

148	54.64	-5.60002	20.0008	-0.00756468	0.730581	293.15	293.15	0	327.924	327.924	0.0743501	0.0743445

149	54.81	-5.68592	20.0008	-0.00768032	0.733559	293.15	293.15	0	328.091	328.091	0.0743893	0.0743843

150	54.98	-5.7843	20.0008	-0.00781279	0.738245	293.15	293.15	0	328.26	328.26	0.0744293	0.0744247

151	55.15	-5.88771	20.0008	-0.00795207	0.741863	293.15	293.15	0	328.428	328.428	0.0744679	0.074463

152	55.31	-5.90755	20.0008	-0.00797846	0.74509	293.15	293.15	0	328.601	328.601	0.0745075	0.0745021

153	55.48	-5.95146	20.0008	-0.00803735	0.749455	293.15	293.15	0	328.765	328.765	0.0745467	0.0745421

154	55.65	-5.95777	20.0008	-0.00804546	0.754352	293.15	293.15	0	328.926	328.926	0.0745855	0.0745817

155	55.82	-5.96181	20.0008	-0.00805052	0.759135	293.15	293.15	0	329.086	329.086	0.0746237	0.07462

156	55.99	-5.99623	19.9956	-0.00809658	0.760445	293.15	293.15	0	329.263	329.263	0.0746638	0.0746599

157	56.16	-6.0814	20.0008	-0.00821115	0.766343	293.15	293.15	0	329.432	329.432	0.0747033	0.0747

158	56.32	-6.13127	20.0008	-0.00827809	0.772056	293.15	293.15	0	329.596	329.596	0.0747402	0.0747378

159	56.49	-6.18278	19.9956	-0.00834721	0.77446	293.15	293.15	0	329.753	329.753	0.0747801	0.0747778

160	56.66	-6.27635	20.0008	-0.0084731	0.7807	293.15	293.15	0	329.919	329.919	0.0748192	0.074817

161	56.83	-6.39908	20.0008	-0.00863834	0.784149	293.15	293.15	0	330.101	330.101	0.0748582	0.0748569

162	56.99	-6.53275	20.0008	-0.00881833	0.790951	293.15	293.15	0	330.266	330.266	0.0748972	0.0748961

163	57.16	-6.69446	20.0008	-0.00903618	0.794281	293.15	293.15	0	330.421	330.421	0.0749351	0.0749343

164	57.33	-6.86637	20.0008	-0.00926775	0.79769	293.15	293.15	0	330.594	330.594	0.0749743	0.074974

165	57.5	-6.98844	20.0008	-0.00943202	0.79987	293.15	293.15	0	330.757	330.757	0.0750138	0.0750141

166	57.66	-7.2043	20.0008	-0.00972288	0.808955	293.15	293.15	0	330.931	330.931	0.0750519	0.0750523

167	57.83	-7.48967	20.0008	-0.0101075	0.815201	293.15	293.15	0	331.096	331.096	0.0750898	0.0750911

168	57.99	-7.83408	20.0008	-0.0105718	0.817453	293.15	293.15	0	331.259	331.259	0.0751282	0.0751298

169	58.16	-8.35159	20.0008	-0.0112695	0.824511	293.15	293.15	0	331.425	331.425	0.075166	0.0751691

170	58.32	-8.92419	20.005	-0.0120416	0.835507	293.15	293.15	0	331.596	331.596	0.0752036	0.0752076

171	58.49	-9.6183	20.0112	-0.0129775	0.841721	293.15	293.15	0	331.762	331.762	0.075241	0.0752466

172	58.66	-10.4616	20.0019	-0.0141146	0.850964	293.15	293.15	0	331.933	331.933	0.0752783	0.0752857

173	58.82	-11.4735	20.0008	-0.0154792	0.864348	293.15	293.15	0	332.092	332.092	0.0753131	0.0753234

174	58.98	-12.8215	20.0039	-0.0172969	0.877901	293.15	293.15	0	332.265	332.265	0.0753494	0.0753623

175	59.14	-14.5086	20.0112	-0.0195719	0.892977	293.15	293.15	0	332.426	332.426	0.0753842	0.0753998

176	59.3	-16.5409	20.0039	-0.0223124	0.909699	293.15	293.15	0	332.596	332.596	0.0754181	0.0754373

177	59.47	-19.0394	20.0008	-0.0256814	0.9286	293.15	293.15	0	332.763	332.763	0.075452	0.0754756

178	59.63	-21.9555	20.0008	-0.0296133	0.948761	293.15	293.15	0	332.924	332.924	0.0754842	0.0755133

179	59.79	-25.3292	20.0008	-0.034162	0.973771	293.15	293.15	0	333.089	333.089	0.0755174	0.0755523

180	59.96	-28.9918	20.0008	-0.0390999	0.998139	293.15	293.15	0	333.256	333.256	0.0755498	0.0755904

181	60.12	-32.9235	19.9946	-0.0444001	1.02579	293.15	293.15	0	333.436	333.436	0.0755823	0.0756293

182	60.29	-36.9987	19.9904	-0.0498933	1.04909	293.15	293.15	0	333.593	333.593	0.075616	0.0756688

183	60.47	-41.0506	20.0008	-0.0553545	1.06872	293.15	293.15	0	333.756	333.756	0.0756516	0.0757095

184	60.64	-44.9171	20.0008	-0.060565	1.0925	293.15	293.15	0	333.921	333.921	0.075688	0.0757511

185	60.82	-48.6883	20.0008	-0.0656464	1.11271	293.15	293.15	0	334.095	334.095	0.075725	0.0757933

186	61.01	-52.2454	20.0008	-0.0704385	1.12811	293.15	293.15	0	334.258	334.258	0.0757642	0.0758369

187	61.2	-55.67	20.0008	-0.0750513	1.14659	293.15	293.15	0	334.431	334.431	0.0758048	0.0758813

188	61.39	-58.6952	20.0008	-0.0791252	1.15715	293.15	293.15	0	334.604	334.604	0.075846	0.0759253

189	61.59	-61.3844	20.0008	-0.0827455	1.16719	293.15	293.15	0	334.768	334.768	0.0758885	0.0759721

190	61.78	-63.531	20.0008	-0.0856341	1.17137	293.15	293.15	0	334.925	334.925	0.0759321	0.0760166

191	61.97	-65.341	20.0008	-0.0880687	1.18049	293.15	293.15	0	335.097	335.097	0.075976	0.0760616

192	62.17	-66.7947	20.0008	-0.0900228	1.18545	293.15	293.15	0	335.262	335.262	0.07602	0.0761071

193	62.36	-67.8685	20.0008	-0.0914647	1.18935	293.15	293.15	0	335.435	335.435	0.0760638	0.0761519

194	62.55	-68.592	20.0008	-0.0924342	1.18824	293.15	293.15	0	335.6	335.6	0.0761101	0.0761979

195	62.74	-69.0028	20.0008	-0.0929825	1.19011	293.15	293.15	0	335.756	335.756	0.0761546	0.0762421

196	62.93	-69.1182	20.0008	-0.0931327	1.19192	293.15	293.15	0	335.935	335.935	0.0761991	0.0762862

197	63.12	-69.0491	20.0008	-0.0930342	1.19011	293.15	293.15	0	336.086	336.086	0.0762433	0.0763303

198	63.3	-68.8579	20.0008	-0.0927716	1.18864	293.15	293.15	0	336.259	336.259	0.0762858	0.0763724

199	63.49	-68.4613	20.0008	-0.092232	1.18584	293.15	293.15	0	336.427	336.427	0.07633	0.076416

200	63.67	-67.9351	20.0008	-0.0915181	1.19016	293.15	293.15	0	336.599	336.599	0.0763731	0.0764585

201	63.85	-67.3068	20.0008	-0.0906668	1.18409	293.15	293.15	0	336.754	336.754	0.0764157	0.0764998

202	64.02	-66.5849	20.0008	-0.0896895	1.1802	293.15	293.15	0	336.919	336.919	0.0764591	0.0765414

203	64.2	-65.7991	20.0008	-0.0886263	1.17967	293.15	293.15	0	337.091	337.091	0.0765005	0.076583

204	64.37	-64.9062	20.0008	-0.087419	1.17865	293.15	293.15	0	337.266	337.266	0.0765431	0.0766233

205	64.55	-63.7809	20.0008	-0.0858989	1.17628	293.15	293.15	0	337.421	337.421	0.0765855	0.0766641

206	64.72	-62.4678	20.0008	-0.0841261	1.16932	293.15	293.15	0	337.594	337.594	0.0766278	0.076704

207	64.89	-60.9847	20.0008	-0.0821246	1.16479	293.15	293.15	0	337.758	337.758	0.0766695	0.0767438

208	65.06	-59.5097	20.0008	-0.0801342	1.16358	293.15	293.15	0	337.931	337.931	0.0767107	0.0767829

209	65.22	-58.066	20.0008	-0.0781863	1.16027	293.15	293.15	0	338.104	338.104	0.0767508	0.0768216

210	65.39	-56.6388	20.0008	-0.0762607	1.15634	293.15	293.15	0	338.259	338.259	0.0767911	0.0768606

211	65.55	-55.0743	20.0008	-0.0741505	1.15042	293.15	293.15	0	338.425	338.425	0.0768324	0.076899

212	65.72	-53.2601	20.0008	-0.0717043	1.14682	293.15	293.15	0	338.596	338.596	0.076875	0.0769387

213	65.89	-51.3049	20.0008	-0.0690684	1.13735	293.15	293.15	0	338.763	338.763	0.0769168	0.0769779

214	66.06	-49.0863	20.0008	-0.0660782	1.13006	293.15	293.15	0	338.936	338.936	0.0769594	0.0770175

215	66.23	-46.5972	20.0008	-0.0627245	1.11912	293.15	293.15	0	339.084	339.084	0.0770021	0.0770559

216	66.39	-43.4546	20.0008	-0.0584912	1.10239	293.15	293.15	0	339.253	339.253	0.0770479	0.077095

217	66.57	-39.3571	20.0008	-0.0529731	1.0788	293.15	293.15	0	339.43	339.43	0.077096	0.0771356

218	66.74	-34.5676	20.0008	-0.0465242	1.05461	293.15	293.15	0	339.599	339.599	0.0771444	0.0771766

219	66.91	-29.5283	20.0008	-0.0397397	1.03125	293.15	293.15	0	339.767	339.767	0.0771917	0.0772162

220	67.07	-24.5453	19.9967	-0.0330319	1.01148	293.15	293.15	0	339.933	339.933	0.0772353	0.077254

221	67.23	-20.108	20.0091	-0.0270592	1.00322	293.15	293.15	0	340.088	340.088	0.0772753	0.07729

222	67.38	-16.1664	20.0008	-0.0217539	0.993455	293.15	293.15	0	340.255	340.255	0.0773136	0.0773254

223	67.52	-13.0365	20.0008	-0.0175415	0.986503	293.15	293.15	0	340.434	340.434	0.0773492	0.0773572

224	67.66	-10.3772	20.0008	-0.0139627	0.985503	293.15	293.15	0	340.603	340.603	0.0773839	0.0773903

225	67.79	-8.34319	20.0008	-0.0112254	0.989089	293.15	293.15	0	340.755	340.755	0.077416	0.0774212

226	67.92	-6.77621	20.0008	-0.00911677	0.994443	293.15	293.15	0	340.928	340.928	0.0774471	0.0774513

227	68.06	-5.49398	20.0008	-0.00739135	1.00021	293.15	293.15	0	341.092	341.092	0.0774795	0.0774833

228	68.19	-4.71016	20.0008	-0.00633657	1.00929	293.15	293.15	0	341.258	341.258	0.0775107	0.0775149

229	68.33	-4.18902	20.0008	-0.00563524	1.01715	293.15	293.15	0	341.438	341.438	0.0775442	0.0775477

230	68.48	-3.80273	20.0008	-0.00511537	1.02468	293.15	293.15	0	341.595	341.595	0.0775772	0.0775811

231	68.62	-3.58539	20.0008	-0.0048228	1.03132	293.15	293.15	0	341.759	341.759	0.0776102	0.0776141

232	68.77	-3.46223	20.0008	-0.00465692	1.03624	293.15	293.15	0	341.932	341.932	0.0776455	0.0776495

233	68.92	-3.44488	20.0008	-0.00463338	1.04707	293.15	293.15	0	342.096	342.096	0.0776795	0.0776838

234	69.07	-3.43495	20.0008	-0.00461981	1.05208	293.15	293.15	0	342.27	342.27	0.0777157	0.0777199

235	69.23	-3.39751	20.0008	-0.00456924	1.05878	293.15	293.15	0	342.435	342.435	0.0777514	0.0777563

236	69.38	-3.48285	20.0008	-0.00468379	1.06668	293.15	293.15	0	342.598	342.598	0.0777869	0.0777927

237	69.55	-3.63324	20.0008	-0.00488579	1.0725	293.15	293.15	0	342.756	342.756	0.0778248	0.0778313

238	69.71	-3.73543	20.0008	-0.00502297	1.07788	293.15	293.15	0	342.929	342.929	0.0778618	0.077868

239	69.87	-3.82754	20.0008	-0.00514657	1.08224	293.15	293.15	0	343.099	343.099	0.0779001	0.077906

240	70.03	-3.94106	20.0008	-0.00529895	1.08716	293.15	293.15	0	343.269	343.269	0.0779376	0.077944

241	70.2	-4.02184	19.9987	-0.00540731	1.09245	293.15	293.15	0	343.424	343.424	0.0779755	0.077982

242	70.36	-4.08485	19.9925	-0.00549175	1.10117	293.15	293.15	0	343.591	343.591	0.0780136	0.0780203

243	70.52	-4.12125	20.0008	-0.00554042	1.10593	293.15	293.15	0	343.761	343.761	0.0780509	0.0780577

244	70.69	-4.20549	20.0008	-0.00565338	1.11032	293.15	293.15	0	343.929	343.929	0.0780894	0.0780968

245	70.86	-4.32177	20.0008	-0.00580939	1.11494	293.15	293.15	0	344.091	344.091	0.0781282	0.0781362

246	71.02	-4.44416	20.0008	-0.00597362	1.12229	293.15	293.15	0	344.266	344.266	0.0781665	0.078174

247	71.19	-4.50402	20.0008	-0.00605377	1.1267	293.15	293.15	0	344.437	344.437	0.0782061	0.0782135

248	71.35	-4.51213	20.0008	-0.00606436	1.13014	293.15	293.15	0	344.594	344.594	0.0782445	0.0782522

249	71.52	-4.5116	20.0008	-0.00606335	1.13402	293.15	293.15	0	344.758	344.758	0.0782835	0.0782913

250	71.69	-4.53116	20.0008	-0.00608934	1.1414	293.15	293.15	0	344.922	344.922	0.0783216	0.07833

251	71.86	-4.56687	20.0008	-0.00613701	1.14469	293.15	293.15	0	345.095	345.095	0.0783605	0.0783697

252	72.03	-4.58652	20.0008	-0.00616309	1.14544	293.15	293.15	0	345.259	345.259	0.0784002	0.0784095

253	72.19	-4.62429	20.0008	-0.00621354	1.15147	293.15	293.15	0	345.425	345.425	0.0784385	0.0784478

254	72.36	-4.61959	20.0008	-0.0062069	1.15635	293.15	293.15	0	345.596	345.596	0.078478	0.0784873

255	72.53	-4.6158	20.0008	-0.0062015	1.16106	293.15	293.15	0	345.762	345.762	0.0785168	0.0785261

256	72.7	-4.5956	20.0008	-0.00617405	1.1634	293.15	293.15	0	345.936	345.936	0.0785554	0.0785651

257	72.86	-4.53369	20.0008	-0.00609056	1.16728	293.15	293.15	0	346.09	346.09	0.0785942	0.078604

258	73.03	-4.44413	20.0008	-0.00596995	1.17598	293.15	293.15	0	346.257	346.257	0.0786327	0.0786425

259	73.2	-4.41892	20.0008	-0.00593579	1.17978	293.15	293.15	0	346.43	346.43	0.0786712	0.0786812

260	73.37	-4.43666	20.0008	-0.00595932	1.18182	293.15	293.15	0	346.59	346.59	0.0787107	0.0787206

261	73.53	-4.46564	20.0008	-0.00599794	1.18498	293.15	293.15	0	346.75	346.75	0.0787491	0.0787596

262	73.71	-4.4773	20.0008	-0.00601329	1.1934	293.15	293.15	0	346.927	346.927	0.0787887	0.0787999

263	73.87	-4.46942	20.0029	-0.00600241	1.19776	293.15	293.15	0	347.096	347.096	0.0788266	0.0788378

264	74.04	-4.48536	20.0112	-0.00602351	1.19827	293.15	293.15	0	347.27	347.27	0.0788666	0.0788773

265	74.21	-4.5132	20.0039	-0.00606058	1.20243	293.15	293.15	0	347.434	347.434	0.0789059	0.0789169

266	74.37	-4.50537	20.0008	-0.00604977	1.20849	293.15	293.15	0	347.592	347.592	0.0789437	0.078955

267	74.54	-4.45376	20.0008	-0.00598016	1.20863	293.15	293.15	0	347.755	347.755	0.0789845	0.0789948

268	74.71	-4.42538	20.0008	-0.00594177	1.21512	293.15	293.15	0	347.928	347.928	0.0790224	0.0790329

269	74.87	-4.36836	20.0008	-0.00586492	1.21973	293.15	293.15	0	348.094	348.094	0.0790601	0.0790712

270	75.04	-4.26478	20.0008	-0.00572556	1.22919	293.15	293.15	0	348.256	348.256	0.0790987	0.0791093

271	75.2	-4.18708	20.0008	-0.00562097	1.23256	293.15	293.15	0	348.422	348.422	0.0791372	0.079148

272	75.37	-4.15624	20.0008	-0.00557928	1.23576	293.15	293.15	0	348.587	348.587	0.0791763	0.0791881

273	75.54	-4.17421	19.9956	-0.00560312	1.23838	293.15	293.15	0	348.759	348.759	0.0792144	0.0792263

274	75.71	-4.22599	19.9904	-0.00567233	1.24178	293.15	293.15	0	348.933	348.933	0.0792535	0.0792654

275	75.88	-4.34039	20.0008	-0.00582559	1.25063	293.15	293.15	0	349.096	349.096	0.0792921	0.0793049

276	76.04	-4.3119	20.0008	-0.00578707	1.2514	293.15	293.15	0	349.27	349.27	0.0793311	0.0793434

277	76.21	-4.24138	20.0008	-0.00569212	1.25615	293.15	293.15	0	349.426	349.426	0.0793703	0.0793832

278	76.38	-4.23185	20.0008	-0.00567906	1.26226	293.15	293.15	0	349.59	349.59	0.0794082	0.0794208

279	76.54	-4.19574	20.0008	-0.00563032	1.26573	293.15	293.15	0	349.764	349.764	0.079447	0.0794599

280	76.71	-4.20356	20.0008	-0.00564053	1.26871	293.15	293.15	0	349.926	349.926	0.0794863	0.0794987

281	76.88	-4.25582	19.9977	-0.00571036	1.27284	293.15	293.15	0	350.085	350.085	0.0795245	0.0795384

282	77.05	-4.2777	19.9935	-0.00573943	1.27741	293.15	293.15	0	350.263	350.263	0.0795637	0.0795773

283	77.21	-4.28589	20.0008	-0.00575013	1.28599	293.15	293.15	0	350.431	350.431	0.079602	0.0796154

284	77.38	-4.27832	20.0008	-0.00573967	1.28777	293.15	293.15	0	350.595	350.595	0.0796415	0.0796553

285	77.55	-4.29625	20.0008	-0.00576344	1.29235	293.15	293.15	0	350.768	350.768	0.0796798	0.0796944

286	77.71	-4.31234	20.0008	-0.00578474	1.29641	293.15	293.15	0	350.929	350.929	0.0797177	0.079732

287	77.89	-4.29116	20.0008	-0.00575604	1.30085	293.15	293.15	0	351.089	351.089	0.0797569	0.0797719

288	78.05	-4.25884	20.0008	-0.0057124	1.30581	293.15	293.15	0	351.266	351.266	0.0797961	0.0798099

289	78.21	-4.21199	20.0008	-0.00564928	1.30908	293.15	293.15	0	351.419	351.419	0.0798341	0.0798485

290	78.39	-4.16954	20.0008	-0.00559205	1.31442	293.15	293.15	0	351.594	351.594	0.0798733	0.0798883

291	78.55	-4.14164	20.0008	-0.00555436	1.32044	293.15	293.15	0	351.765	351.765	0.0799121	0.0799263

292	78.72	-4.08898	20.0008	-0.00548345	1.32297	293.15	293.15	0	351.93	351.93	0.0799515	0.0799662

293	78.88	-4.09236	19.9956	-0.00548772	1.33084	293.15	293.15	0	352.086	352.086	0.0799884	0.0800037

294	79.05	-4.14426	20.0008	-0.00555703	1.3325	293.15	293.15	0	352.268	352.268	0.0800282	0.0800427

295	79.22	-4.22132	20.0008	-0.00566007	1.33486	293.15	293.15	0	352.433	352.433	0.0800671	0.0800823

296	79.39	-4.2084	20.0008	-0.00564248	1.34475	293.15	293.15	0	352.597	352.597	0.0801046	0.0801203

297	79.55	-4.13648	20.0008	-0.00554577	1.34753	293.15	293.15	0	352.77	352.77	0.0801439	0.0801595

298	79.72	-4.08425	20.0008	-0.00547546	1.35201	293.15	293.15	0	352.933	352.933	0.0801814	0.0801974

299	79.89	-4.11554	20.0008	-0.00551713	1.35996	293.15	293.15	0	353.099	353.099	0.0802204	0.0802365

300	80.06	-4.13344	19.9914	-0.00554084	1.36281	293.15	293.15	0	353.262	353.262	0.0802593	0.0802762

301	80.22	-4.16715	19.9956	-0.00558576	1.36445	293.15	293.15	0	353.421	353.421	0.0802986	0.0803153

302	80.39	-4.16785	19.9935	-0.00558642	1.36906	293.15	293.15	0	353.599	353.599	0.0803377	0.0803536

303	80.56	-4.1185	20.0008	-0.00552	1.37352	293.15	293.15	0	353.767	353.767	0.0803758	0.0803925

304	80.73	-4.06128	19.9987	-0.00544303	1.37556	293.15	293.15	0	353.932	353.932	0.0804154	0.0804318

305	80.89	-4.04791	19.9904	-0.00542483	1.38418	293.15	293.15	0	354.092	354.092	0.0804535	0.0804698

306	81.06	-4.08487	19.9925	-0.00547409	1.38867	293.15	293.15	0	354.261	354.261	0.0804913	0.0805082

307	81.23	-4.06633	20.0008	-0.00544897	1.39256	293.15	293.15	0	354.434	354.434	0.0805303	0.0805475

308	81.39	-3.98897	20.0008	-0.00534504	1.39695	293.15	293.15	0	354.593	354.593	0.0805686	0.0805853

309	81.56	-3.93302	20.0008	-0.0052698	1.402	293.15	293.15	0	354.754	354.754	0.080608	0.0806248

310	81.73	-3.93471	20.0008	-0.0052718	1.40848	293.15	293.15	0	354.928	354.928	0.0806462	0.0806639

311	81.89	-3.95131	19.9998	-0.00529379	1.41423	293.15	293.15	0	355.095	355.095	0.0806838	0.0807017

312	82.06	-3.9842	19.9966	-0.00533756	1.41516	293.15	293.15	0	355.267	355.267	0.0807238	0.080742

313	82.23	-3.99749	20.0008	-0.00535511	1.42253	293.15	293.15	0	355.422	355.422	0.0807631	0.08078

314	82.4	-4.06963	20.0008	-0.00545147	1.42554	293.15	293.15	0	355.586	355.586	0.0808018	0.0808196

315	82.57	-4.13272	19.9956	-0.0055357	1.42967	293.15	293.15	0	355.759	355.759	0.0808403	0.0808586

316	82.73	-4.09717	19.9904	-0.00548782	1.43483	293.15	293.15	0	355.932	355.932	0.0808774	0.0808958

317	82.9	-3.99999	20.0008	-0.00535738	1.44059	293.15	293.15	0	356.096	356.096	0.0809172	0.080935

318	83.06	-3.81661	20.0008	-0.00511152	1.44718	293.15	293.15	0	356.269	356.269	0.0809551	0.0809733

319	83.23	-3.65128	20.0008	-0.00488984	1.44927	293.15	293.15	0	356.427	356.427	0.080994	0.0810126

320	83.4	-3.69945	20.0008	-0.00495409	1.45244	293.15	293.15	0	356.591	356.591	0.0810334	0.0810526

321	83.57	-3.76452	20.0008	-0.00504098	1.46025	293.15	293.15	0	356.764	356.764	0.0810714	0.0810905

322	83.74	-3.78593	20.0008	-0.0050694	1.45959	293.15	293.15	0	356.926	356.926	0.0811115	0.0811303

323	83.91	-3.82276	19.9956	-0.00511846	1.46499	293.15	293.15	0	357.093	357.093	0.0811495	0.0811691

324	84.07	-3.79558	20.0008	-0.00508181	1.46973	293.15	293.15	0	357.263	357.263	0.0811881	0.081207

325	84.24	-3.74913	20.0008	-0.00501937	1.4757	293.15	293.15	0	357.431	357.431	0.0812268	0.0812456

326	84.4	-3.68641	20.0029	-0.00493516	1.4828	293.15	293.15	0	357.597	357.597	0.0812645	0.0812832

327	84.57	-3.57358	20.0091	-0.00478387	1.48424	293.15	293.15	0	357.755	357.755	0.0813036	0.0813229

328	84.74	-3.56022	20.0008	-0.00476574	1.48889	293.15	293.15	0	357.925	357.925	0.0813425	0.0813617

329	84.9	-3.58253	20.0008	-0.00479536	1.49694	293.15	293.15	0	358.099	358.099	0.0813806	0.0814004

330	85.07	-3.56183	20.0008	-0.00476742	1.50112	293.15	293.15	0	358.266	358.266	0.0814186	0.0814384

331	85.24	-3.56936	20.0008	-0.00477726	1.50445	293.15	293.15	0	358.435	358.435	0.0814574	0.0814774

332	85.4	-3.55023	20.0008	-0.00475141	1.50928	293.15	293.15	0	358.602	358.602	0.0814961	0.0815163

333	85.57	-3.51507	20.0008	-0.00470412	1.51497	293.15	293.15	0	358.758	358.758	0.0815352	0.081555

334	85.74	-3.46122	20.0008	-0.00463182	1.52176	293.15	293.15	0	358.929	358.929	0.0815727	0.0815935

335	85.9	-3.41009	20.0008	-0.00456317	1.52673	293.15	293.15	0	359.086	359.086	0.0816113	0.0816322

336	86.07	-3.35694	20.0008	-0.00449182	1.53022	293.15	293.15	0	359.259	359.259	0.0816494	0.0816709

337	86.24	-3.33826	20.0008	-0.00446661	1.53242	293.15	293.15	0	359.423	359.423	0.0816892	0.0817095

338	86.41	-3.34608	20.0008	-0.00447683	1.54129	293.15	293.15	0	359.597	359.597	0.0817274	0.0817487

339	86.57	-3.42214	20.0008	-0.00457837	1.54357	293.15	293.15	0	359.761	359.761	0.0817662	0.0817874

340	86.74	-3.48673	20.0008	-0.00466456	1.54834	293.15	293.15	0	359.926	359.926	0.0818047	0.0818262

341	86.9	-3.47354	20.0008	-0.00464668	1.5552	293.15	293.15	0	360.088	360.088	0.0818423	0.0818634

342	87.07	-3.37331	20.0008	-0.00451237	1.55968	293.15	293.15	0	360.255	360.255	0.0818815	0.0819027

343	87.24	-3.31253	20.0008	-0.00443084	1.56484	293.15	293.15	0	360.428	360.428	0.0819199	0.0819413

344	87.41	-3.33432	20.0008	-0.00445977	1.56802	293.15	293.15	0	360.592	360.592	0.0819582	0.0819802

345	87.58	-3.383	20.0008	-0.00452464	1.57739	293.15	293.15	0	360.763	360.763	0.0819969	0.0820196

346	87.74	-3.37092	20.005	-0.00450827	1.57891	293.15	293.15	0	360.938	360.938	0.0820357	0.0820583

347	87.91	-3.35336	20.0112	-0.00448454	1.58004	293.15	293.15	0	361.086	361.086	0.0820754	0.0820976

348	88.08	-3.32516	20.0081	-0.00444661	1.58689	293.15	293.15	0	361.255	361.255	0.0821136	0.0821366

349	88.25	-3.29704	20.0008	-0.00440879	1.59308	293.15	293.15	0	361.432	361.432	0.0821521	0.0821746

350	88.41	-3.30048	20.0008	-0.00441316	1.59855	293.15	293.15	0	361.602	361.602	0.0821905	0.0822133

351	88.58	-3.28309	20.0008	-0.00438969	1.60239	293.15	293.15	0	361.77	361.77	0.0822289	0.0822512

352	88.75	-3.33726	20.0008	-0.0044619	1.60636	293.15	293.15	0	361.935	361.935	0.0822673	0.0822904

353	88.91	-3.39558	20.0008	-0.00453965	1.61151	293.15	293.15	0	362.091	362.091	0.0823053	0.0823286

354	89.08	-3.36893	20.0029	-0.00450379	1.61874	293.15	293.15	0	362.258	362.258	0.0823442	0.0823679

355	89.25	-3.33343	20.0112	-0.0044561	1.62548	293.15	293.15	0	362.431	362.431	0.0823824	0.082407

356	89.41	-3.32452	20.0112	-0.00444398	1.62844	293.15	293.15	0	362.594	362.594	0.0824204	0.0824445

357	89.58	-3.28105	20.005	-0.00438564	1.6334	293.15	293.15	0	362.767	362.767	0.0824596	0.0824838

358	89.75	-3.2757	20.0008	-0.00437828	1.63829	293.15	293.15	0	362.923	362.923	0.082498	0.0825224

359	89.92	-3.31397	20.0008	-0.0044292	1.64327	293.15	293.15	0	363.088	363.088	0.0825371	0.0825611

360	90.08	-3.2995	20.0008	-0.00440964	1.64867	293.15	293.15	0	363.262	363.262	0.0825753	0.0825999

361	90.25	-3.24131	20.0112	-0.00433166	1.65022	293.15	293.15	0	363.434	363.434	0.0826141	0.0826384

362	90.42	-3.2088	20.0008	-0.004288	1.65852	293.15	293.15	0	363.607	363.607	0.0826521	0.0826769

363	90.59	-3.1595	20.0008	-0.00422191	1.66177	293.15	293.15	0	363.755	363.755	0.082691	0.0827164

364	90.75	-3.19689	20.0008	-0.00427165	1.66547	293.15	293.15	0	363.919	363.919	0.0827303	0.0827546

365	90.92	-3.24663	20.0008	-0.00433789	1.66933	293.15	293.15	0	364.092	364.092	0.0827682	0.0827937

366	91.09	-3.26351	20.0008	-0.00436023	1.67756	293.15	293.15	0	364.263	364.263	0.0828068	0.0828318

367	91.26	-3.29348	20.0008	-0.00440005	1.68046	293.15	293.15	0	364.429	364.429	0.0828455	0.0828714

368	91.42	-3.25665	20.0008	-0.00435063	1.68566	293.15	293.15	0	364.594	364.594	0.0828842	0.0829096

369	91.59	-3.13864	20.0008	-0.00419276	1.68952	293.15	293.15	0	364.757	364.757	0.0829223	0.0829478

370	91.76	-3.07534	20.0008	-0.00410801	1.6973	293.15	293.15	0	364.923	364.923	0.0829603	0.0829864

371	91.92	-3.05915	20.0008	-0.00408617	1.70308	293.15	293.15	0	365.096	365.096	0.0829986	0.0830247

372	92.09	-3.06774	20.0008	-0.00409745	1.70676	293.15	293.15	0	365.266	365.266	0.0830379	0.0830635

373	92.26	-3.10543	20.0008	-0.00414757	1.71062	293.15	293.15	0	365.433	365.433	0.083076	0.0831021

374	92.43	-3.12109	20.0008	-0.00416828	1.71378	293.15	293.15	0	365.603	365.603	0.0831147	0.0831412

375	92.59	-3.12157	20.0008	-0.00416871	1.72086	293.15	293.15	0	365.764	365.764	0.0831535	0.0831799

376	92.76	-3.09581	20.0008	-0.0041341	1.72507	293.15	293.15	0	365.927	365.927	0.0831916	0.0832182

377	92.93	-3.05779	20.0008	-0.00408313	1.72959	293.15	293.15	0	366.101	366.101	0.08323	0.0832564

378	93.09	-3.03127	20.0008	-0.00404752	1.7337	293.15	293.15	0	366.259	366.259	0.0832684	0.083295

379	93.26	-3.0162	20.0008	-0.00402718	1.73961	293.15	293.15	0	366.421	366.421	0.0833076	0.0833334

380	93.43	-2.96876	20.0008	-0.00396365	1.74632	293.15	293.15	0	366.595	366.595	0.0833454	0.0833723

381	93.59	-2.91637	20.0008	-0.00389351	1.75152	293.15	293.15	0	366.761	366.761	0.0833832	0.0834106

382	93.76	-2.8873	20.0008	-0.0038545	1.75887	293.15	293.15	0	366.923	366.923	0.0834221	0.0834494

383	93.92	-2.84917	20.0008	-0.00380341	1.76393	293.15	293.15	0	367.089	367.089	0.0834601	0.0834868

384	94.09	-2.78989	20.0008	-0.00372409	1.76805	293.15	293.15	0	367.253	367.253	0.0834989	0.0835259

385	94.26	-2.78706	20.0112	-0.00372012	1.77245	293.15	293.15	0	367.426	367.426	0.0835375	0.0835648

386	94.43	-2.77248	20.0008	-0.00370049	1.77612	293.15	293.15	0	367.599	367.599	0.0835755	0.083603

387	94.59	-2.80012	20.0008	-0.00373719	1.78302	293.15	293.15	0	367.763	367.763	0.0836144	0.0836418

388	94.76	-2.82341	20.0008	-0.00376809	1.7878	293.15	293.15	0	367.936	367.936	0.0836522	0.0836802

389	94.93	-2.84793	20.0008	-0.00380061	1.79222	293.15	293.15	0	368.084	368.084	0.083691	0.0837189

390	95.1	-2.8626	20.0008	-0.00382	1.79638	293.15	293.15	0	368.256	368.256	0.0837301	0.0837575

391	95.26	-2.82448	20.0008	-0.00376895	1.80393	293.15	293.15	0	368.438	368.438	0.0837678	0.0837956

392	95.43	-2.75829	20.0008	-0.00368044	1.80809	293.15	293.15	0	368.594	368.594	0.0838066	0.0838347

393	95.59	-2.72032	20.0008	-0.00362959	1.81343	293.15	293.15	0	368.751	368.751	0.0838444	0.0838727

394	95.77	-2.67729	20.0008	-0.00357199	1.81559	293.15	293.15	0	368.924	368.924	0.0838836	0.083912

395	95.93	-2.62112	20.0008	-0.00349688	1.82437	293.15	293.15	0	369.094	369.094	0.0839216	0.0839502

396	96.1	-2.60254	20.0008	-0.00347192	1.82772	293.15	293.15	0	369.262	369.262	0.0839603	0.0839885

397	96.27	-2.65717	20.0008	-0.00354461	1.83162	293.15	293.15	0	369.434	369.434	0.0839994	0.0840283

398	96.44	-2.68741	20.0008	-0.00358477	1.83633	293.15	293.15	0	369.595	369.595	0.0840381	0.0840675

399	96.6	-2.67905	20.0008	-0.00357345	1.84196	293.15	293.15	0	369.756	369.756	0.0840759	0.0841055

400	96.77	-2.6787	20.0008	-0.00357281	1.8493	293.15	293.15	0	369.929	369.929	0.0841135	0.0841436

401	96.93	-2.64211	20.0008	-0.00352382	1.85253	293.15	293.15	0	370.097	370.097	0.0841522	0.0841815

402	97.1	-2.61575	20.0008	-0.00348849	1.85986	293.15	293.15	0	370.266	370.266	0.084191	0.0842207

403	97.27	-2.5817	20.0008	-0.00344291	1.86422	293.15	293.15	0	370.422	370.422	0.084229	0.0842602

404	97.44	-2.60142	20.0008	-0.00346903	1.86777	293.15	293.15	0	370.589	370.589	0.0842684	0.0842981

405	97.61	-2.67989	20.0008	-0.00357349	1.87415	293.15	293.15	0	370.76	370.76	0.0843065	0.0843371

406	97.78	-2.73648	20.0008	-0.00364876	1.88114	293.15	293.15	0	370.934	370.934	0.0843442	0.0843756

407	97.94	-2.71757	20.0008	-0.00362337	1.88616	293.15	293.15	0	371.097	371.097	0.0843833	0.0844141

408	98.11	-2.67004	20.0008	-0.00355982	1.88882	293.15	293.15	0	371.254	371.254	0.0844216	0.0844527

409	98.28	-2.57724	20.0008	-0.00343592	1.89467	293.15	293.15	0	371.418	371.418	0.0844601	0.0844909

410	98.44	-2.48655	20.0008	-0.00331486	1.89807	293.15	293.15	0	371.591	371.591	0.0844986	0.0845287

411	98.6	-2.48629	20.0008	-0.00331435	1.90859	293.15	293.15	0	371.755	371.755	0.0845358	0.0845668

412	98.77	-2.51693	20.0008	-0.00335502	1.91164	293.15	293.15	0	371.938	371.938	0.0845744	0.0846059

413	98.94	-2.51181	20.0008	-0.00334803	1.91566	293.15	293.15	0	372.085	372.085	0.0846126	0.0846441

414	99.11	-2.45394	20.0008	-0.00327074	1.91916	293.15	293.15	0	372.259	372.259	0.0846512	0.0846822

415	99.28	-2.43962	19.9956	-0.00325148	1.92809	293.15	293.15	0	372.429	372.429	0.0846905	0.0847217

416	99.44	-2.48568	20.0008	-0.0033127	1.93459	293.15	293.15	0	372.595	372.595	0.0847271	0.0847594

417	99.61	-2.51239	20.0008	-0.00334813	1.93622	293.15	293.15	0	372.769	372.769	0.0847663	0.0847981

418	99.77	-2.52966	20.0008	-0.00337098	1.94283	293.15	293.15	0	372.931	372.931	0.0848047	0.0848363

419	99.94	-2.5301	20.0008	-0.00337139	1.94475	293.15	293.15	0	373.085	373.085	0.0848434	0.0848755

420	100.11	-2.57126	20.0008	-0.00342606	1.86842	293.15	293.15	0	373.065	373.065	0.0848822	0.0849145

421	100.25	-2.65682	19.9987	-0.00353993	1.74731	293.15	293.15	0	372.908	372.908	0.084913	0.0849449

422	100.3	-2.38816	19.9925	-0.00318193	1.63903	293.15	293.15	0	372.741	372.741	0.0849265	0.0849567

423	100.27	-1.17513	20.0008	-0.00156573	1.55503	293.15	293.15	0	372.588	372.588	0.0849253	0.0849509

424	100.19	0.822998	20.0008	0.00109658	1.47492	293.15	293.15	0	372.412	372.412	0.0849105	0.0849322

425	100.06	3.25233	20.0008	0.00433362	1.41332	293.15	293.15	0	372.241	372.241	0.0848859	0.0849029

426	99.9	5.92482	20.0008	0.00789502	1.36322	293.15	293.15	0	372.075	372.075	0.084853	0.0848652

427	99.71	8.68609	20.0008	0.0115752	1.33144	293.15	293.15	0	371.919	371.919	0.0848125	0.084821

428	99.5	11.3769	20.0008	0.0151618	1.3022	293.15	293.15	0	371.747	371.747	0.0847688	0.0847739

429	99.28	13.8042	20.0008	0.018398	1.27967	293.15	293.15	0	371.574	371.574	0.08472	0.0847227

430	99.05	15.8422	20.0008	0.0211155	1.26815	293.15	293.15	0	371.4	371.4	0.0846689	0.0846704

431	98.82	17.6054	20.0008	0.0234674	1.25783	293.15	293.15	0	371.245	371.245	0.0846185	0.084617

432	98.59	19.11	20.0008	0.0254748	1.25057	293.15	293.15	0	371.08	371.08	0.0845653	0.0845623

433	98.35	20.2391	20.0008	0.0269818	1.24819	293.15	293.15	0	370.906	370.906	0.084511	0.0845083

434	98.12	21.0168	20.0008	0.0280205	1.25226	293.15	293.15	0	370.735	370.735	0.0844595	0.0844557

435	97.89	21.5343	20.0008	0.0287124	1.25171	293.15	293.15	0	370.585	370.585	0.0844072	0.084403

436	97.68	21.8783	20.0008	0.029173	1.25093	293.15	293.15	0	370.412	370.412	0.0843581	0.0843539

437	97.46	22.1518	20.0008	0.0295396	1.24954	293.15	293.15	0	370.243	370.243	0.0843081	0.0843038

438	97.25	22.2572	20.0008	0.029682	1.2536	293.15	293.15	0	370.075	370.075	0.084259	0.0842549

439	97.04	22.2288	20.0008	0.029646	1.25522	293.15	293.15	0	369.909	369.909	0.0842119	0.0842067

440	96.85	22.1315	19.9987	0.0295179	1.25852	293.15	293.15	0	369.751	369.751	0.084166	0.0841624

441	96.65	21.9335	19.9925	0.0292555	1.2588	293.15	293.15	0	369.581	369.581	0.0841209	0.0841171

442	96.46	21.6135	20.0008	0.0288304	1.25884	293.15	293.15	0	369.408	369.408	0.0840761	0.0840723

443	96.27	21.2768	20.0008	0.0283829	1.26051	293.15	293.15	0	369.24	369.24	0.0840334	0.0840295

444	96.09	21.0221	20.0008	0.0280446	1.26157	293.15	293.15	0	369.071	369.071	0.0839902	0.0839879

445	95.91	20.8651	20.0008	0.0278366	1.25779	293.15	293.15	0	368.914	368.914	0.0839486	0.0839461

446	95.74	20.5721	20.0008	0.0274471	1.25628	293.15	293.15	0	368.748	368.748	0.083908	0.0839062

447	95.56	20.2884	20.0008	0.0270701	1.25348	293.15	293.15	0	368.576	368.576	0.0838673	0.0838651

448	95.39	20.1273	20.0008	0.0268565	1.24889	293.15	293.15	0	368.403	368.403	0.0838275	0.0838258

449	95.22	19.9794	20.0008	0.0266606	1.24509	293.15	293.15	0	368.24	368.24	0.0837882	0.0837851

450	95.05	19.7528	20.0008	0.0263595	1.24293	293.15	293.15	0	368.083	368.083	0.0837487	0.083746

451	94.88	19.5146	20.0008	0.026043	1.24055	293.15	293.15	0	367.918	367.918	0.083709	0.083707

452	94.7	19.318	20.0008	0.025782	1.23987	293.15	293.15	0	367.746	367.746	0.0836695	0.0836672

453	94.54	19.2069	20.0008	0.0256349	1.23238	293.15	293.15	0	367.582	367.582	0.0836306	0.0836288

454	94.37	19.1486	19.9956	0.0255585	1.22492	293.15	293.15	0	367.408	367.408	0.0835937	0.0835901

455	94.21	19.114	20.0008	0.0255135	1.2249	293.15	293.15	0	367.235	367.235	0.0835546	0.0835519

456	94.04	19.0859	20.0008	0.0254773	1.22017	293.15	293.15	0	367.071	367.071	0.0835165	0.083514

457	93.87	19.0406	20.006	0.025418	1.21303	293.15	293.15	0	366.914	366.914	0.083478	0.0834747

458	93.7	19.0716	20.0008	0.0254608	1.20893	293.15	293.15	0	366.743	366.743	0.0834397	0.0834359

459	93.54	19.074	20.0008	0.0254653	1.20381	293.15	293.15	0	366.577	366.577	0.0834012	0.0833976

460	93.37	18.9916	20.0008	0.0253564	1.19947	293.15	293.15	0	366.403	366.403	0.0833629	0.0833594

461	93.2	18.9228	20.0008	0.0252659	1.1931	293.15	293.15	0	366.24	366.24	0.0833244	0.0833209

462	93.03	18.8246	20.0008	0.025136	1.19154	293.15	293.15	0	366.077	366.077	0.0832852	0.0832813

463	92.87	18.7526	20.0008	0.0250412	1.186	293.15	293.15	0	365.91	365.91	0.0832474	0.083243

464	92.7	18.7388	20.0008	0.025024	1.18335	293.15	293.15	0	365.74	365.74	0.0832082	0.083204

465	92.53	18.7781	20.0008	0.0250778	1.17728	293.15	293.15	0	365.572	365.572	0.0831697	0.083165

466	92.37	18.7883	20.0039	0.0250926	1.17329	293.15	293.15	0	365.409	365.409	0.0831314	0.083127

467	92.2	18.7727	20.0112	0.025073	1.16995	293.15	293.15	0	365.252	365.252	0.0830918	0.0830881

468	92.03	18.7526	20.0039	0.0250475	1.16488	293.15	293.15	0	365.084	365.084	0.0830545	0.0830502

469	91.87	18.7309	20.0008	0.0250197	1.15803	293.15	293.15	0	364.914	364.914	0.0830168	0.0830124

470	91.7	18.7012	20.0008	0.0249812	1.15316	293.15	293.15	0	364.737	364.737	0.0829775	0.0829735

471	91.54	18.6637	20.0008	0.0249324	1.15018	293.15	293.15	0	364.569	364.569	0.0829391	0.0829358

472	91.36	18.5954	20.0008	0.0248424	1.14766	293.15	293.15	0	364.413	364.413	0.0829002	0.0828956

473	91.2	18.5631	20.0008	0.0248005	1.13884	293.15	293.15	0	364.245	364.245	0.0828627	0.0828585

474	91.03	18.5284	20.0008	0.0247554	1.13337	293.15	293.15	0	364.074	364.074	0.0828239	0.0828187

475	90.86	18.5322	20.0008	0.0247618	1.12873	293.15	293.15	0	363.917	363.917	0.0827854	0.08278

476	90.7	18.5802	20.0008	0.0248271	1.12413	293.15	293.15	0	363.735	363.735	0.0827474	0.0827417

477	90.53	18.6124	20.0008	0.0248713	1.12262	293.15	293.15	0	363.588	363.588	0.0827083	0.0827028

478	90.36	18.6522	20.0008	0.0249258	1.11545	293.15	293.15	0	363.413	363.413	0.0826703	0.082664

479	90.2	18.636	20.0008	0.0249054	1.10938	293.15	293.15	0	363.243	363.243	0.082631	0.082626

480	90.03	18.5706	20.0008	0.0248192	1.10688	293.15	293.15	0	363.077	363.077	0.0825923	0.0825876

481	89.87	18.5127	20.0008	0.024743	1.09947	293.15	293.15	0	362.904	362.904	0.0825545	0.0825495

482	89.7	18.4734	20.0008	0.0246918	1.0949	293.15	293.15	0	362.742	362.742	0.0825161	0.0825104

483	89.53	18.4104	20.0008	0.0246088	1.08987	293.15	293.15	0	362.574	362.574	0.0824777	0.0824718

484	89.36	18.4244	20.0008	0.0246288	1.08545	293.15	293.15	0	362.404	362.404	0.0824393	0.0824324

485	89.19	18.4936	20.0008	0.0247225	1.08274	293.15	293.15	0	362.237	362.237	0.0823999	0.0823935

486	89.03	18.5615	20.0008	0.0248146	1.07735	293.15	293.15	0	362.082	362.082	0.0823614	0.0823551

487	88.86	18.5873	20.0008	0.0248503	1.07187	293.15	293.15	0	361.916	361.916	0.0823227	0.0823158

488	88.69	18.5741	20.0008	0.0248339	1.07019	293.15	293.15	0	361.749	361.749	0.0822834	0.0822765

489	88.52	18.5276	20.0008	0.0247731	1.06707	293.15	293.15	0	361.579	361.579	0.0822446	0.0822374

490	88.35	18.471	20.0008	0.0246986	1.05909	293.15	293.15	0	361.402	361.402	0.0822069	0.0821996

491	88.19	18.4486	20.0008	0.0246699	1.05472	293.15	293.15	0	361.233	361.233	0.0821687	0.0821613

492	88.02	18.4874	20.0008	0.024723	1.05324	293.15	293.15	0	361.077	361.077	0.0821292	0.0821215

493	87.85	18.469	20.0008	0.0246996	1.04668	293.15	293.15	0	360.91	360.91	0.0820907	0.0820831

494	87.69	18.3423	20.0008	0.0245314	1.04052	293.15	293.15	0	360.745	360.745	0.0820525	0.0820447

495	87.52	18.2584	20.0008	0.0244204	1.03604	293.15	293.15	0	360.574	360.574	0.0820137	0.082006

496	87.35	18.2666	20.0008	0.0244326	1.03141	293.15	293.15	0	360.408	360.408	0.0819751	0.0819677

497	87.18	18.3136	20.0008	0.0244967	1.02832	293.15	293.15	0	360.253	360.253	0.081936	0.0819282

498	87.01	18.3735	20.0008	0.0245781	1.02441	293.15	293.15	0	360.071	360.071	0.081898	0.081889

499	86.85	18.3505	20.0008	0.0245485	1.01677	293.15	293.15	0	359.907	359.907	0.0818596	0.0818514

500	86.68	18.3087	19.9904	0.0244938	1.01461	293.15	293.15	0	359.741	359.741	0.0818206	0.0818127

501	86.52	18.2749	20.0091	0.0244498	1.01141	293.15	293.15	0	359.586	359.586	0.0817824	0.0817741

502	86.35	18.2629	20.0029	0.024435	1.00493	293.15	293.15	0	359.415	359.415	0.0817429	0.081735

503	86.18	18.2442	19.9904	0.0244112	1.00101	293.15	293.15	0	359.249	359.249	0.0817046	0.0816964

504	86.01	18.2093	19.9956	0.0243658	0.997362	293.15	293.15	0	359.069	359.069	0.0816659	0.0816576

505	85.84	18.176	19.9946	0.0243224	0.994075	293.15	293.15	0	358.902	358.902	0.0816265	0.0816177

506	85.68	18.1572	20.0008	0.0242984	0.989689	293.15	293.15	0	358.737	358.737	0.0815885	0.0815793

507	85.51	18.1707	19.9956	0.0243178	0.983413	293.15	293.15	0	358.576	358.576	0.0815503	0.0815405

508	85.34	18.1944	20.0008	0.0243508	0.977763	293.15	293.15	0	358.408	358.408	0.0815116	0.0815016

509	85.17	18.1882	20.0008	0.0243437	0.975945	293.15	293.15	0	358.235	358.235	0.0814721	0.0814632

510	85.01	18.1618	20.0008	0.0243095	0.96822	293.15	293.15	0	358.075	358.075	0.0814349	0.0814251

511	84.84	18.1736	20.0008	0.0243265	0.964458	293.15	293.15	0	357.915	357.915	0.0813955	0.0813853

512	84.67	18.2263	20.0008	0.0243983	0.961619	293.15	293.15	0	357.741	357.741	0.0813561	0.081346

513	84.51	18.2311	19.9987	0.024406	0.957523	293.15	293.15	0	357.573	357.573	0.0813187	0.0813082

514	84.34	18.2059	19.9914	0.0243735	0.9539	293.15	293.15	0	357.413	357.413	0.0812802	0.0812693

515	84.17	18.1407	20.0008	0.0242875	0.945421	293.15	293.15	0	357.248	357.248	0.0812421	0.0812301

516	84	18.0971	20.0008	0.0242303	0.942574	293.15	293.15	0	357.081	357.081	0.0812032	0.081191

517	83.83	18.0721	20.0008	0.0241981	0.935684	293.15	293.15	0	356.9	356.9	0.0811639	0.0811524

518	83.67	18.0585	20.0008	0.024181	0.931281	293.15	293.15	0	356.744	356.744	0.0811262	0.0811148

519	83.5	18.0508	20.0008	0.0241719	0.928397	293.15	293.15	0	356.589	356.589	0.0810862	0.0810743

520	83.33	18.0878	20.0008	0.0242227	0.925135	293.15	293.15	0	356.407	356.407	0.0810469	0.0810348

521	83.16	18.1082	20.0008	0.0242512	0.921542	293.15	293.15	0	356.243	356.243	0.0810085	0.0809972

522	82.99	18.0501	20.0008	0.0241746	0.919249	293.15	293.15	0	356.079	356.079	0.0809691	0.0809577

523	82.83	18.0793	20.0008	0.024215	0.912506	293.15	293.15	0	355.905	355.905	0.0809306	0.0809194

524	82.66	18.1022	20.0008	0.0242469	0.909096	293.15	293.15	0	355.741	355.741	0.0808923	0.0808808

525	82.49	18.0969	20.0008	0.0242409	0.90455	293.15	293.15	0	355.585	355.585	0.0808541	0.080842

526	82.33	18.0762	20.0008	0.0242144	0.899294	293.15	293.15	0	355.404	355.404	0.080816	0.0808039

527	82.16	18.0912	20.0008	0.0242358	0.89756	293.15	293.15	0	355.246	355.246	0.080777	0.0807644

528	81.99	18.0835	20.0008	0.0242267	0.88801	293.15	293.15	0	355.076	355.076	0.0807384	0.0807251

529	81.83	18.084	20.0008	0.0242285	0.885813	293.15	293.15	0	354.909	354.909	0.0807003	0.0806871

530	81.66	18.1208	20.0008	0.0242791	0.881054	293.15	293.15	0	354.739	354.739	0.0806609	0.0806475

531	81.49	18.131	20.0008	0.024294	0.879794	293.15	293.15	0	354.579	354.579	0.080622	0.080609

532	81.32	18.1011	20.0008	0.0242552	0.875795	293.15	293.15	0	354.405	354.405	0.0805822	0.0805687

533	81.16	18.0662	20.0008	0.0242096	0.870105	293.15	293.15	0	354.238	354.238	0.0805442	0.0805319

534	80.99	18.0636	20.0008	0.0242074	0.866988	293.15	293.15	0	354.077	354.077	0.0805057	0.0804925

535	80.82	18.0452	20.0008	0.0241839	0.861557	293.15	293.15	0	353.911	353.911	0.0804672	0.0804531

536	80.65	17.9988	20.0008	0.0241229	0.85626	293.15	293.15	0	353.746	353.746	0.0804285	0.0804151

537	80.48	17.9612	20.0008	0.0240737	0.852441	293.15	293.15	0	353.575	353.575	0.0803893	0.0803755

538	80.32	17.9038	20.0008	0.0239981	0.845331	293.15	293.15	0	353.408	353.408	0.0803517	0.0803374

539	80.15	17.926	20.0008	0.024029	0.843017	293.15	293.15	0	353.253	353.253	0.0803122	0.0802978

540	79.98	17.8998	19.9956	0.0239952	0.842072	293.15	293.15	0	353.08	353.08	0.0802733	0.0802591

541	79.82	17.8736	20.0008	0.0239612	0.833334	293.15	293.15	0	352.916	352.916	0.080235	0.0802203

542	79.65	17.8108	20.0008	0.0238782	0.829959	293.15	293.15	0	352.743	352.743	0.0801964	0.0801816

543	79.48	17.8237	20.0008	0.0238967	0.825748	293.15	293.15	0	352.561	352.561	0.0801583	0.0801431

544	79.31	17.8992	20.0008	0.0239991	0.820127	293.15	293.15	0	352.404	352.404	0.0801192	0.0801037

545	79.14	17.9686	20.0008	0.0240935	0.816796	293.15	293.15	0	352.24	352.24	0.08008	0.0800644

546	78.98	18.0139	19.9977	0.0241553	0.815112	293.15	293.15	0	352.078	352.078	0.0800415	0.0800257

547	78.81	17.9308	19.9935	0.0240451	0.811212	293.15	293.15	0	351.91	351.91	0.0800017	0.0799863

548	78.64	17.877	20.0008	0.0239742	0.806522	293.15	293.15	0	351.741	351.741	0.0799639	0.0799477

549	78.48	17.863	20.0008	0.0239567	0.800221	293.15	293.15	0	351.573	351.573	0.0799247	0.0799089

550	78.31	17.8003	20.0008	0.0238737	0.799057	293.15	293.15	0	351.409	351.409	0.0798855	0.0798709

551	78.14	17.7214	19.9977	0.0237692	0.793245	293.15	293.15	0	351.235	351.235	0.0798471	0.0798312

552	77.97	17.7047	19.9925	0.0237479	0.789632	293.15	293.15	0	351.075	351.075	0.0798086	0.0797922

553	77.81	17.727	20.0008	0.0237791	0.786052	293.15	293.15	0	350.914	350.914	0.0797696	0.0797538

554	77.64	17.8064	20.0008	0.0238867	0.779773	293.15	293.15	0	350.738	350.738	0.079731	0.0797144

555	77.47	17.8549	20.0008	0.023953	0.777167	293.15	293.15	0	350.568	350.568	0.0796923	0.0796757

556	77.31	17.9084	19.9998	0.024026	0.773707	293.15	293.15	0	350.413	350.413	0.0796536	0.0796371

557	77.14	17.8931	19.9914	0.0240067	0.767372	293.15	293.15	0	350.247	350.247	0.0796149	0.0795979

558	76.97	17.8834	20.0008	0.0239949	0.765872	293.15	293.15	0	350.082	350.082	0.0795756	0.079559

559	76.8	17.8883	20.0008	0.0240026	0.759267	293.15	293.15	0	349.901	349.901	0.0795365	0.0795195

560	76.63	17.8484	20.0008	0.0239503	0.756467	293.15	293.15	0	349.744	349.744	0.0794974	0.0794806

561	76.47	17.7913	19.9904	0.023875	0.753935	293.15	293.15	0	349.58	349.58	0.079459	0.0794422

562	76.3	17.746	20.0008	0.0238153	0.745267	293.15	293.15	0	349.407	349.407	0.0794216	0.0794042

563	76.14	17.7066	20.0008	0.0237637	0.742219	293.15	293.15	0	349.243	349.243	0.0793827	0.0793653

564	75.97	17.6661	20.0008	0.0237105	0.738955	293.15	293.15	0	349.079	349.079	0.0793438	0.0793261

565	75.8	17.6249	20.0008	0.0236563	0.732958	293.15	293.15	0	348.906	348.906	0.0793044	0.0792864

566	75.63	17.6306	20.0008	0.0236652	0.729478	293.15	293.15	0	348.742	348.742	0.0792666	0.0792474

567	75.47	17.6317	20.0008	0.0236679	0.726395	293.15	293.15	0	348.576	348.576	0.0792274	0.0792093

568	75.3	17.6239	20.0008	0.0236586	0.721184	293.15	293.15	0	348.405	348.405	0.0791889	0.0791701

569	75.13	17.6622	20.0008	0.0237112	0.717428	293.15	293.15	0	348.239	348.239	0.0791499	0.0791305

570	74.96	17.6369	20.0008	0.0236784	0.710861	293.15	293.15	0	348.073	348.073	0.0791104	0.0790922

571	74.8	17.5671	19.9977	0.0235859	0.70907	293.15	293.15	0	347.912	347.912	0.0790724	0.0790538

572	74.63	17.5693	19.9935	0.0235901	0.703884	293.15	293.15	0	347.743	347.743	0.0790334	0.0790146

573	74.46	17.6073	20.0008	0.0236423	0.702232	293.15	293.15	0	347.571	347.571	0.0789942	0.0789753

574	74.29	17.6602	20.0008	0.0237145	0.696851	293.15	293.15	0	347.411	347.411	0.0789556	0.0789362

575	74.12	17.722	20.0008	0.0237988	0.692576	293.15	293.15	0	347.251	347.251	0.0789166	0.0788966

576	73.96	17.6979	20.0008	0.0237675	0.688984	293.15	293.15	0	347.073	347.073	0.0788784	0.0788582

577	73.79	17.6521	20.0008	0.0237073	0.688671	293.15	293.15	0	346.904	346.904	0.0788385	0.0788183

578	73.62	17.6174	20.0008	0.0236618	0.682174	293.15	293.15	0	346.738	346.738	0.0787992	0.0787797

579	73.45	17.5821	20.0008	0.0236156	0.679137	293.15	293.15	0	346.584	346.584	0.0787606	0.078741

580	73.28	17.5575	19.9998	0.0235838	0.674408	293.15	293.15	0	346.417	346.417	0.0787225	0.0787013

581	73.12	17.4874	19.9914	0.0234908	0.666749	293.15	293.15	0	346.236	346.236	0.0786845	0.0786638

582	72.95	17.487	20.0008	0.0234915	0.663213	293.15	293.15	0	346.08	346.08	0.0786448	0.0786242

583	72.78	17.5788	20.0008	0.023616	0.659019	293.15	293.15	0	345.916	345.916	0.0786058	0.0785849

584	72.61	17.683	20.0008	0.0237571	0.656587	293.15	293.15	0	345.743	345.743	0.078567	0.0785455

585	72.45	17.7499	20.0008	0.0238483	0.654323	293.15	293.15	0	345.579	345.579	0.0785281	0.0785071

586	72.28	17.661	20.0008	0.02373	0.647499	293.15	293.15	0	345.405	345.405	0.0784897	0.0784689

587	72.12	17.5577	20.0008	0.0235924	0.645137	293.15	293.15	0	345.233	345.233	0.0784503	0.0784294

588	71.95	17.5233	20.0008	0.0235474	0.639832	293.15	293.15	0	345.067	345.067	0.078412	0.0783903

589	71.78	17.5105	20.0008	0.0235313	0.638667	293.15	293.15	0	344.912	344.912	0.0783729	0.078351

590	71.61	17.4521	19.9966	0.0234541	0.630811	293.15	293.15	0	344.74	344.74	0.0783345	0.0783126

591	71.45	17.391	19.9904	0.0233731	0.628501	293.15	293.15	0	344.581	344.581	0.0782949	0.0782735

592	71.28	17.3875	19.9904	0.0233695	0.624591	293.15	293.15	0	344.413	344.413	0.0782563	0.0782338

593	71.11	17.392	19.9987	0.0233769	0.622164	293.15	293.15	0	344.245	344.245	0.0782166	0.0781942

594	70.94	17.4328	20.0008	0.0234329	0.618185	293.15	293.15	0	344.071	344.071	0.0781778	0.0781554

595	70.77	17.4578	20.0008	0.0234677	0.612413	293.15	293.15	0	343.907	343.907	0.0781393	0.078117

596	70.61	17.4129	20.0008	0.0234084	0.609557	293.15	293.15	0	343.746	343.746	0.0781008	0.0780791

597	70.44	17.2994	20.0008	0.023257	0.607351	293.15	293.15	0	343.574	343.574	0.0780614	0.0780396

598	70.27	17.2283	20.0019	0.0231626	0.601454	293.15	293.15	0	343.408	343.408	0.0780234	0.0780005

599	70.11	17.236	20.0102	0.0231742	0.596612	293.15	293.15	0	343.238	343.238	0.0779837	0.077961

600	69.93	17.2725	20.0008	0.0232244	0.592659	293.15	293.15	0	343.072	343.072	0.0779447	0.0779213

601	69.77	17.28	19.9904	0.0232357	0.589619	293.15	293.15	0	342.917	342.917	0.0779065	0.0778833

602	69.6	17.2655	20.0008	0.0232174	0.586494	293.15	293.15	0	342.744	342.744	0.0778672	0.0778437

603	69.44	17.24	20.0008	0.0231842	0.584181	293.15	293.15	0	342.572	342.572	0.0778285	0.0778051

604	69.27	17.2341	20.0008	0.0231774	0.575484	293.15	293.15	0	342.407	342.407	0.0777905	0.0777664

605	69.1	17.1682	20.0008	0.0230901	0.571809	293.15	293.15	0	342.234	342.234	0.0777515	0.0777275

606	68.94	17.1133	20.0008	0.0230173	0.571503	293.15	293.15	0	342.068	342.068	0.0777126	0.077689

607	68.76	17.1515	20.0008	0.0230699	0.566743	293.15	293.15	0	341.903	341.903	0.0776728	0.0776483

608	68.6	17.2004	20.0008	0.0231369	0.562152	293.15	293.15	0	341.741	341.741	0.0776335	0.0776093

609	68.43	17.2123	20.0008	0.023154	0.56044	293.15	293.15	0	341.583	341.583	0.0775942	0.0775699

610	68.26	17.1889	20.0008	0.0231237	0.555051	293.15	293.15	0	341.41	341.41	0.0775559	0.0775313

611	68.1	17.1941	20.0008	0.0231318	0.551494	293.15	293.15	0	341.246	341.246	0.0775177	0.0774926

612	67.93	17.225	20.0008	0.0231746	0.5458	293.15	293.15	0	341.077	341.077	0.0774791	0.0774529

613	67.76	17.2793	20.0008	0.0232488	0.542184	293.15	293.15	0	340.915	340.915	0.0774403	0.0774148

614	67.59	17.3621	20.0008	0.0233615	0.539702	293.15	293.15	0	340.748	340.748	0.0774004	0.0773748

615	67.43	17.3555	20.0008	0.0233538	0.537859	293.15	293.15	0	340.579	340.579	0.0773614	0.077336

616	67.26	17.3094	20.0008	0.0232928	0.533604	293.15	293.15	0	340.402	340.402	0.0773232	0.0772973

617	67.09	17.2816	20.0008	0.0232567	0.529303	293.15	293.15	0	340.248	340.248	0.0772837	0.0772575

618	66.92	17.2865	20.0008	0.0232644	0.525607	293.15	293.15	0	340.075	340.075	0.077244	0.0772179

619	66.75	17.2984	20.0008	0.0232817	0.521684	293.15	293.15	0	339.909	339.909	0.0772056	0.0771793

620	66.59	17.3113	20.0008	0.0233001	0.512311	293.15	293.15	0	339.738	339.738	0.0771675	0.0771403

621	66.42	17.34	19.9956	0.0233399	0.510926	293.15	293.15	0	339.582	339.582	0.0771284	0.0771014

622	66.25	17.3467	19.9904	0.0233501	0.508128	293.15	293.15	0	339.408	339.408	0.0770889	0.0770619

623	66.09	17.3109	20.0008	0.0233031	0.505227	293.15	293.15	0	339.244	339.244	0.0770504	0.0770238

624	65.92	17.2468	20.0008	0.0232181	0.50324	293.15	293.15	0	339.071	339.071	0.0770112	0.0769845

625	65.75	17.2529	20.0008	0.0232274	0.496619	293.15	293.15	0	338.914	338.914	0.0769726	0.0769457

626	65.59	17.2447	20.0008	0.0232176	0.493552	293.15	293.15	0	338.743	338.743	0.0769343	0.0769066

627	65.42	17.3182	19.9914	0.0233178	0.490519	293.15	293.15	0	338.577	338.577	0.0768951	0.0768666

628	65.25	17.3917	19.9904	0.0234178	0.483363	293.15	293.15	0	338.404	338.404	0.0768555	0.0768284

629	65.09	17.3941	19.9998	0.0234222	0.481875	293.15	293.15	0	338.24	338.24	0.0768167	0.0767897

630	64.91	17.3354	20.0008	0.0233444	0.479319	293.15	293.15	0	338.077	338.077	0.0767772	0.076749

631	64.75	17.3167	20.0008	0.0233204	0.476524	293.15	293.15	0	337.919	337.919	0.076738	0.0767103

632	64.57	17.292	19.9977	0.0232883	0.474742	293.15	293.15	0	337.74	337.74	0.0766985	0.0766695

633	64.41	17.2932	19.9904	0.0232912	0.467018	293.15	293.15	0	337.572	337.572	0.0766594	0.0766311

634	64.24	17.2171	19.9904	0.0231897	0.464497	293.15	293.15	0	337.4	337.4	0.076621	0.0765928

635	64.08	17.1241	19.9977	0.0230657	0.462318	293.15	293.15	0	337.252	337.252	0.076582	0.0765538

636	63.91	17.114	20.0008	0.0230533	0.456862	293.15	293.15	0	337.084	337.084	0.0765435	0.0765157

637	63.75	17.1252	20.0008	0.0230695	0.450487	293.15	293.15	0	336.915	336.915	0.0765057	0.0764769

638	63.58	17.1918	20.0008	0.0231603	0.447975	293.15	293.15	0	336.741	336.741	0.0764671	0.0764378

639	63.41	17.1916	20.0008	0.0231613	0.445253	293.15	293.15	0	336.577	336.577	0.0764273	0.0763983

640	63.24	17.134	20.0008	0.0230849	0.438048	293.15	293.15	0	336.41	336.41	0.0763891	0.0763595

641	63.08	17.0661	20.0008	0.0229945	0.436588	293.15	293.15	0	336.24	336.24	0.0763496	0.0763201

642	62.91	17.091	20.0008	0.0230292	0.432908	293.15	293.15	0	336.072	336.072	0.0763104	0.0762811

643	62.74	17.1518	20.0008	0.0231124	0.43006	293.15	293.15	0	335.91	335.91	0.0762717	0.076242

644	62.57	17.1979	20.0008	0.0231757	0.425712	293.15	293.15	0	335.737	335.737	0.0762319	0.076202

645	62.4	17.2055	20.0008	0.0231872	0.42125	293.15	293.15	0	335.571	335.571	0.0761925	0.0761626

646	62.24	17.1631	20.0008	0.0231311	0.419333	293.15	293.15	0	335.409	335.409	0.0761534	0.0761237

647	62.07	17.0501	20.0008	0.02298	0.417445	293.15	293.15	0	335.243	335.243	0.0761135	0.0760838

648	61.9	16.9685	19.9904	0.0228711	0.412427	293.15	293.15	0	335.079	335.079	0.0760761	0.0760455

649	61.74	16.9422	19.9956	0.0228369	0.406455	293.15	293.15	0	334.905	334.905	0.0760373	0.0760068

650	61.57	16.9303	19.9904	0.022822	0.405341	293.15	293.15	0	334.733	334.733	0.0759972	0.0759667

651	61.4	16.9833	19.9904	0.0228946	0.402341	293.15	293.15	0	334.569	334.569	0.0759587	0.0759274

652	61.23	17.0187	20.005	0.0229435	0.39996	293.15	293.15	0	334.403	334.403	0.0759188	0.0758885

653	61.06	17.0676	20.0112	0.0230105	0.396344	293.15	293.15	0	334.247	334.247	0.0758802	0.0758488

654	60.9	17.0624	19.9966	0.0230047	0.390667	293.15	293.15	0	334.077	334.077	0.0758408	0.0758106

655	60.73	16.9899	20.0008	0.0229082	0.388626	293.15	293.15	0	333.911	333.911	0.0758028	0.0757723

656	60.56	16.9744	20.0008	0.0228884	0.381714	293.15	293.15	0	333.737	333.737	0.0757639	0.0757325

657	60.39	16.9607	20.0008	0.0228711	0.379576	293.15	293.15	0	333.573	333.573	0.075725	0.0756927

658	60.23	16.9476	20.0008	0.0228546	0.3759	293.15	293.15	0	333.411	333.411	0.0756856	0.0756548

659	60.06	16.9147	20.0008	0.0228113	0.373161	293.15	293.15	0	333.252	333.252	0.0756468	0.0756153

660	59.89	16.8583	20.0008	0.0227365	0.369241	293.15	293.15	0	333.074	333.074	0.0756076	0.0755758

661	59.73	16.8076	20.0008	0.0226692	0.364106	293.15	293.15	0	332.906	332.906	0.075569	0.0755369

662	59.56	16.7448	20.0008	0.0225856	0.363609	293.15	293.15	0	332.742	332.742	0.0755286	0.075497

663	59.39	16.7118	20.0008	0.0225423	0.359038	293.15	293.15	0	332.569	332.569	0.0754903	0.0754585

664	59.23	16.7138	19.9987	0.0225461	0.353403	293.15	293.15	0	332.409	332.409	0.0754513	0.0754192

665	59.06	16.7759	19.9904	0.0226311	0.349683	293.15	293.15	0	332.248	332.248	0.0754122	0.0753801

666	58.89	16.7546	19.9977	0.0226034	0.348121	293.15	293.15	0	332.08	332.08	0.0753732	0.0753412

667	58.72	16.6446	20.0008	0.0224562	0.343324	293.15	293.15	0	331.909	331.909	0.0753339	0.0753014

668	58.56	16.6092	20.0008	0.0224096	0.339711	293.15	293.15	0	331.741	331.741	0.0752958	0.0752631

669	58.39	16.6424	20.0008	0.0224555	0.335732	293.15	293.15	0	331.571	331.571	0.0752555	0.0752224

670	58.22	16.6543	20.0008	0.0224728	0.3313	293.15	293.15	0	331.405	331.405	0.0752167	0.0751834

671	58.05	16.6443	19.9956	0.0224603	0.329099	293.15	293.15	0	331.251	331.251	0.0751777	0.0751437

672	57.88	16.5882	19.9904	0.0223858	0.327262	293.15	293.15	0	331.078	331.078	0.0751385	0.0751041

673	57.72	16.5767	20.0008	0.0223715	0.322658	293.15	293.15	0	330.913	330.913	0.0751004	0.0750661

674	57.55	16.6232	20.006	0.0224354	0.31768	293.15	293.15	0	330.741	330.741	0.0750608	0.0750265

675	57.38	16.706	20.0008	0.0225483	0.312071	293.15	293.15	0	330.575	330.575	0.075022	0.0749869

676	57.23	18.2983	20.0008	0.0246985	0.277985	293.15	293.15	0	330.403	330.403	0.0749971	0.0749521

677	57.11	23.7828	19.9956	0.0321024	0.223749	293.15	293.15	0	330.246	330.246	0.0749851	0.0749234

678	56.99	30.8985	20.0008	0.0417089	0.170062	293.15	293.15	0	330.073	330.073	0.0749685	0.074896

679	56.84	37.8528	20.0008	0.0510984	0.1347	293.15	293.15	0	329.909	329.909	0.0749422	0.0748614

680	56.68	44.1901	20.0008	0.0596564	0.100198	293.15	293.15	0	329.737	329.737	0.0749116	0.0748228

681	56.5	50.1596	20.0008	0.0677188	0.070006	293.15	293.15	0	329.572	329.572	0.0748773	0.0747813

682	56.32	56.0019	19.9946	0.0756105	0.0450651	293.15	293.15	0	329.406	329.406	0.0748416	0.0747382

683	56.13	61.5949	20.0008	0.0831666	0.020159	293.15	293.15	0	329.251	329.251	0.0748053	0.0746944

684	55.93	66.7724	20.0008	0.0901628	0.00133589	293.15	293.15	0	329.081	329.081	0.074765	0.0746477

685	55.73	71.6585	20.0008	0.0967664	-0.0211447	293.15	293.15	0	328.905	328.905	0.0747239	0.0746004

686	55.55	75.9441	20.0008	0.102559	-0.0406682	293.15	293.15	0	328.744	328.744	0.0746845	0.0745569

687	55.37	79.6191	20.0008	0.107528	-0.061375	293.15	293.15	0	328.584	328.584	0.0746451	0.0745145

688	55.2	82.5469	20.0008	0.111488	-0.0881218	293.15	293.15	0	328.407	328.407	0.0746087	0.0744759

689	55.03	84.9624	20.0008	0.114756	-0.114963	293.15	293.15	0	328.238	328.238	0.0745723	0.0744365

690	54.87	86.9294	20.0008	0.117418	-0.14659	293.15	293.15	0	328.071	328.071	0.0745365	0.0743994

691	54.72	88.5788	20.0008	0.119652	-0.175169	293.15	293.15	0	327.915	327.915	0.0745023	0.0743643

692	54.58	89.883	20.0008	0.121419	-0.211846	293.15	293.15	0	327.743	327.743	0.0744688	0.0743297

693	54.43	90.8856	20.0008	0.122779	-0.252401	293.15	293.15	0	327.57	327.57	0.0744366	0.074296

694	54.29	91.6852	20.0008	0.123864	-0.287253	293.15	293.15	0	327.413	327.413	0.0744039	0.0742628

695	54.15	92.0659	20.0008	0.124384	-0.326608	293.15	293.15	0	327.25	327.25	0.0743704	0.0742304

696	54.01	92.0013	20.0008	0.124302	-0.36321	293.15	293.15	0	327.076	327.076	0.0743359	0.0741967

697	53.86	91.4848	20.0008	0.12361	-0.398012	293.15	293.15	0	326.912	326.912	0.0743004	0.0741623

698	53.72	90.7115	20.0008	0.12257	-0.437984	293.15	293.15	0	326.739	326.739	0.0742645	0.0741285

699	53.57	89.7048	20.0008	0.121215	-0.472409	293.15	293.15	0	326.565	326.565	0.074227	0.0740929

700	53.42	88.4737	20.0008	0.119557	-0.5019	293.15	293.15	0	326.411	326.411	0.0741892	0.074057

701	53.26	87.1145	20.0102	0.117726	-0.531787	293.15	293.15	0	326.245	326.245	0.0741499	0.0740202

702	53.1	85.5896	20.0019	0.115671	-0.565631	293.15	293.15	0	326.074	326.074	0.07411	0.0739822

703	52.94	83.9942	20.0008	0.11352	-0.592819	293.15	293.15	0	325.908	325.908	0.0740691	0.0739447

704	52.76	82.215	20.0008	0.111122	-0.615579	293.15	293.15	0	325.737	325.737	0.0740261	0.0739036

705	52.59	80.1845	20.0008	0.108383	-0.633894	293.15	293.15	0	325.578	325.578	0.0739815	0.0738621

706	52.4	77.8199	20.0008	0.105193	-0.649499	293.15	293.15	0	325.414	325.414	0.0739346	0.0738196

707	52.21	75.1138	19.9956	0.101541	-0.657531	293.15	293.15	0	325.241	325.241	0.0738843	0.0737739

708	52.01	72.1591	19.9987	0.0975525	-0.65833	293.15	293.15	0	325.08	325.08	0.0738329	0.073727

709	51.8	68.8705	19.9925	0.0931126	-0.651439	293.15	293.15	0	324.911	324.911	0.0737781	0.0736775

710	51.58	65.2854	20.0008	0.0882715	-0.634681	293.15	293.15	0	324.743	324.743	0.07372	0.0736249

711	51.35	61.4443	20.0008	0.0830839	-0.613696	293.15	293.15	0	324.565	324.565	0.0736603	0.0735709

712	51.1	57.3502	20.0019	0.0775537	-0.582192	293.15	293.15	0	324.406	324.406	0.0735963	0.0735124

713	50.84	53.1847	20.0091	0.0719263	-0.541257	293.15	293.15	0	324.243	324.243	0.0735316	0.0734529

714	50.57	48.8682	19.9914	0.0660942	-0.485518	293.15	293.15	0	324.068	324.068	0.0734621	0.0733894

715	50.3	44.5799	20.0008	0.0602993	-0.426144	293.15	293.15	0	323.914	323.914	0.0733915	0.0733251

716	50.01	40.5719	20.0008	0.0548828	-0.362529	293.15	293.15	0	323.74	323.74	0.0733211	0.0732577

717	49.73	37.0813	20.0008	0.0501653	-0.288165	293.15	293.15	0	323.576	323.576	0.0732507	0.0731902

718	49.44	34.2081	19.9956	0.0462823	-0.211272	293.15	293.15	0	323.413	323.413	0.0731813	0.0731227

719	49.15	31.8089	19.9946	0.0430401	-0.130375	293.15	293.15	0	323.239	323.239	0.0731117	0.0730556

720	48.87	29.9574	20.0008	0.0405383	-0.047191	293.15	293.15	0	323.074	323.074	0.0730453	0.0729898

721	48.6	28.4795	20.0008	0.0385417	0.0410418	293.15	293.15	0	322.909	322.909	0.0729795	0.0729249

722	48.33	27.3193	20.0008	0.0369745	0.128049	293.15	293.15	0	322.738	322.738	0.0729178	0.0728626

723	48.15	26.2294	20.0008	0.0355014	0.176396	293.15	293.15	0	322.587	322.587	0.0728716	0.0728191

724	48.02	24.6918	19.9977	0.0334216	0.216263	293.15	293.15	0	322.41	322.41	0.072838	0.0727889

725	47.92	22.6976	19.9935	0.0307232	0.239316	293.15	293.15	0	322.242	322.242	0.0728122	0.0727663

726	47.85	20.5069	20.0008	0.0277585	0.250376	293.15	293.15	0	322.072	322.072	0.0727916	0.0727492

727	47.78	18.2918	20.0008	0.0247605	0.254825	293.15	293.15	0	321.912	321.912	0.0727728	0.0727334

728	47.72	16.3091	20.0008	0.0220771	0.251451	293.15	293.15	0	321.744	321.744	0.0727562	0.0727191

729	47.65	14.6435	20.0008	0.0198229	0.242189	293.15	293.15	0	321.573	321.573	0.0727398	0.0727033

730	47.58	13.385	19.9998	0.0181196	0.232023	293.15	293.15	0	321.407	321.407	0.0727222	0.0726861

731	47.51	12.5414	19.9904	0.0169781	0.219965	293.15	293.15	0	321.252	321.252	0.0727037	0.0726681

732	47.42	12.0045	20.0008	0.0162517	0.207783	293.15	293.15	0	321.079	321.079	0.0726831	0.0726472

733	47.32	11.7575	20.0008	0.0159177	0.194009	293.15	293.15	0	320.915	320.915	0.0726606	0.0726242

734	47.21	11.6868	20.0008	0.0158226	0.181024	293.15	293.15	0	320.741	320.741	0.072636	0.0725988

735	47.09	11.7948	20.0008	0.0159694	0.170452	293.15	293.15	0	320.568	320.568	0.0726094	0.0725714

736	46.98	12.0264	20.0008	0.0162835	0.16064	293.15	293.15	0	320.414	320.414	0.0725819	0.0725435

737	46.85	12.2983	20.0008	0.0166523	0.148097	293.15	293.15	0	320.248	320.248	0.0725518	0.0725128

738	46.71	12.6672	20.0008	0.0171525	0.139893	293.15	293.15	0	320.076	320.076	0.0725208	0.0724808

739	46.57	13.0911	20.0008	0.0177272	0.131643	293.15	293.15	0	319.91	319.91	0.0724877	0.0724473

740	46.42	13.5269	20.0008	0.0183182	0.121991	293.15	293.15	0	319.735	319.735	0.0724545	0.072413

741	46.27	13.9414	19.9956	0.0188805	0.116721	293.15	293.15	0	319.584	319.584	0.0724198	0.0723769

742	46.12	14.2818	20.0008	0.0193423	0.111242	293.15	293.15	0	319.416	319.416	0.0723836	0.0723418

743	45.97	14.5658	20.0008	0.0197278	0.104591	293.15	293.15	0	319.243	319.243	0.0723477	0.0723056

744	45.81	14.8228	20.0008	0.0200769	0.0976092	293.15	293.15	0	319.074	319.074	0.0723119	0.0722687

745	45.65	15.0371	20.0008	0.0203682	0.0909688	293.15	293.15	0	318.906	318.906	0.0722741	0.0722304

746	45.48	15.2737	20.0008	0.0206896	0.0851982	293.15	293.15	0	318.741	318.741	0.0722368	0.0721925

747	45.32	15.5192	20.0008	0.0210233	0.084062	293.15	293.15	0	318.582	318.582	0.0721977	0.0721535

748	45.16	15.7002	19.9987	0.0212695	0.0789694	293.15	293.15	0	318.412	318.412	0.0721608	0.0721163

749	44.99	15.7891	19.9904	0.0213911	0.0747173	293.15	293.15	0	318.248	318.248	0.0721216	0.0720764

750	44.82	15.9211	19.9925	0.0215709	0.0717638	293.15	293.15	0	318.071	318.071	0.0720816	0.0720361

751	44.66	16.096	20.0008	0.021809	0.0691841	293.15	293.15	0	317.902	317.902	0.0720433	0.0719975

752	44.49	16.2873	20.0008	0.0220693	0.0660627	293.15	293.15	0	317.735	317.735	0.0720035	0.0719578

753	44.32	16.3881	20.0008	0.0222071	0.0618221	293.15	293.15	0	317.579	317.579	0.0719644	0.0719184

754	44.15	16.3862	20.0008	0.0222056	0.0582875	293.15	293.15	0	317.407	317.407	0.0719248	0.0718784

755	43.99	16.3702	20.0008	0.0221851	0.055134	293.15	293.15	0	317.251	317.251	0.0718856	0.0718399

756	43.82	16.3404	20.0008	0.0221458	0.0537997	293.15	293.15	0	317.078	317.078	0.0718465	0.0718009

757	43.65	16.3013	20.0008	0.022094	0.0510724	293.15	293.15	0	316.913	316.913	0.0718075	0.0717608

758	43.48	16.278	20.0008	0.0220635	0.0447046	293.15	293.15	0	316.74	316.74	0.0717686	0.0717213

759	43.32	16.2982	20.0008	0.022092	0.0452825	293.15	293.15	0	316.577	316.577	0.0717282	0.0716817

760	43.15	16.3493	20.0008	0.0221624	0.0412199	293.15	293.15	0	316.394	316.394	0.0716889	0.0716414

761	42.98	16.3354	20.0008	0.0221446	0.0383257	293.15	293.15	0	316.246	316.246	0.0716495	0.0716025

762	42.81	16.3549	20.0008	0.0221723	0.0346738	293.15	293.15	0	316.073	316.073	0.0716105	0.0715627

763	42.64	16.4147	20.0008	0.0222544	0.0325958	293.15	293.15	0	315.909	315.909	0.071571	0.0715228

764	42.48	16.4143	20.0008	0.0222551	0.0343411	293.15	293.15	0	315.737	315.737	0.071531	0.0714833

765	42.31	16.3779	20.0008	0.0222068	0.0286801	293.15	293.15	0	315.572	315.572	0.0714909	0.0714433

766	42.14	16.3915	20.0008	0.0222265	0.0261466	293.15	293.15	0	315.407	315.407	0.0714522	0.0714044

767	41.97	16.3492	20.0008	0.0221702	0.0265347	293.15	293.15	0	315.251	315.251	0.0714116	0.0713636

768	41.8	16.3081	20.0008	0.0221157	0.0251681	293.15	293.15	0	315.081	315.081	0.071372	0.0713241

769	41.63	16.1936	20.0008	0.0219615	0.0246115	293.15	293.15	0	314.914	314.914	0.0713321	0.0712842

770	41.47	16.1211	20.0008	0.0218643	0.0192123	293.15	293.15	0	314.735	314.735	0.0712932	0.0712452

771	41.3	16.0994	20.0008	0.021836	0.016173	293.15	293.15	0	314.583	314.583	0.0712547	0.0712058

772	41.13	16.1278	20.0008	0.0218755	0.0169537	293.15	293.15	0	314.407	314.407	0.0712139	0.0711651

773	40.96	16.1291	20.0008	0.0218784	0.0154847	293.15	293.15	0	314.238	314.238	0.071175	0.0711263

774	40.79	16.1022	20.0008	0.021843	0.0128509	293.15	293.15	0	314.065	314.065	0.0711347	0.0710861

775	40.63	16.1322	19.9998	0.0218849	0.00934362	293.15	293.15	0	313.916	313.916	0.0710967	0.0710469

776	40.46	16.093	19.9914	0.0218327	0.00680155	293.15	293.15	0	313.75	313.75	0.0710581	0.0710088

777	40.3	16.0142	20.0008	0.0217269	-5.03929e-05	293.15	293.15	0	313.579	313.579	0.0710202	0.0709712

778	40.15	15.9235	20.0008	0.0216049	-0.00985934	293.15	293.15	0	313.404	313.404	0.0709835	0.0709345

779	39.99	15.8228	20.0008	0.0214693	-0.0170536	293.15	293.15	0	313.233	313.233	0.070946	0.0708976

780	39.84	15.7397	20.0008	0.0213575	-0.0268295	293.15	293.15	0	313.067	313.067	0.0709107	0.0708617

781	39.69	15.6191	20.0008	0.0211949	-0.0354469	293.15	293.15	0	312.912	312.912	0.0708746	0.0708263

782	39.54	15.4493	20.0008	0.0209654	-0.050727	293.15	293.15	0	312.748	312.748	0.0708391	0.0707905

783	39.39	15.3298	20.0008	0.0208042	-0.0651426	293.15	293.15	0	312.575	312.575	0.070805	0.0707561

784	39.25	15.1906	20.0008	0.0206162	-0.0810107	293.15	293.15	0	312.402	312.402	0.0707709	0.070723

785	39.11	15.0467	20.0008	0.0204218	-0.0981238	293.15	293.15	0	312.238	312.238	0.0707371	0.0706886

786	38.97	14.9281	20.0008	0.0202617	-0.1216	293.15	293.15	0	312.065	312.065	0.0707031	0.0706552

787	38.83	14.8238	20.0008	0.020121	-0.142138	293.15	293.15	0	311.908	311.908	0.0706707	0.0706221

788	38.69	14.7149	20.0008	0.019974	-0.16669	293.15	293.15	0	311.735	311.735	0.0706387	0.0705906

789	38.55	14.6146	20.0008	0.0198387	-0.18813	293.15	293.15	0	311.582	311.582	0.0706059	0.070558

790	38.42	14.4714	20.0008	0.0196451	-0.22053	293.15	293.15	0	311.399	311.399	0.0705752	0.0705267

791	38.29	14.3345	20.0008	0.01946	-0.250573	293.15	293.15	0	311.248	311.248	0.0705445	0.0704963

792	38.16	14.2331	20.0008	0.0193231	-0.286093	293.15	293.15	0	311.075	311.075	0.0705138	0.0704656

793	38.04	14.0676	20.0008	0.0190991	-0.32118	293.15	293.15	0	310.911	310.911	0.0704843	0.0704354

794	37.91	13.9264	20.0008	0.0189081	-0.359591	293.15	293.15	0	310.743	310.743	0.0704544	0.0704063

795	37.79	13.8048	20.0008	0.0187438	-0.403886	293.15	293.15	0	310.573	310.573	0.0704251	0.0703775

796	37.67	13.684	20.0081	0.0185804	-0.446732	293.15	293.15	0	310.408	310.408	0.0703967	0.0703485

797	37.54	13.5751	20.0102	0.0184332	-0.48985	293.15	293.15	0	310.252	310.252	0.0703682	0.0703193

798	37.43	13.5162	20.0008	0.0183539	-0.537	293.15	293.15	0	310.087	310.087	0.0703393	0.0702915

799	37.31	13.4649	20.0008	0.0182849	-0.596614	293.15	293.15	0	309.907	309.907	0.0703117	0.0702634

800	37.19	13.4374	20.0008	0.0182482	-0.647557	293.15	293.15	0	309.75	309.75	0.070284	0.0702358

801	37.08	13.4054	20.0008	0.0182054	-0.704981	293.15	293.15	0	309.585	309.585	0.070257	0.0702094

802	36.97	13.3447	19.9956	0.0181236	-0.767898	293.15	293.15	0	309.412	309.412	0.070231	0.0701827

803	36.86	13.2315	20.0008	0.0179704	-0.834442	293.15	293.15	0	309.248	309.248	0.0702048	0.0701572

804	36.75	13.0862	20.0008	0.0177736	-0.903979	293.15	293.15	0	309.075	309.075	0.0701791	0.0701319

805	36.64	12.9245	20.0008	0.0175546	-0.977168	293.15	293.15	0	308.902	308.902	0.0701539	0.0701065

806	36.54	12.81	20.0008	0.0173996	-1.04724	293.15	293.15	0	308.747	308.747	0.0701294	0.0700817

807	36.43	12.7689	20.0008	0.0173444	-1.12538	293.15	293.15	0	308.581	308.581	0.0701038	0.070056

808	36.33	12.7098	20.0008	0.0172647	-1.20996	293.15	293.15	0	308.41	308.41	0.0700799	0.0700324

809	36.23	12.6234	20.0008	0.0171479	-1.29763	293.15	293.15	0	308.235	308.235	0.0700558	0.0700083

810	36.13	12.5511	19.9977	0.0170502	-1.38458	293.15	293.15	0	308.072	308.072	0.0700322	0.0699845

811	36.03	12.4474	19.9935	0.0169097	-1.47254	293.15	293.15	0	307.914	307.914	0.0700085	0.0699616

812	35.93	12.3233	20.0008	0.0167416	-1.57225	293.15	293.15	0	307.741	307.741	0.0699856	0.0699381

813	35.84	12.1554	20.0008	0.0165141	-1.67331	293.15	293.15	0	307.571	307.571	0.0699628	0.0699155

814	35.74	11.9876	20.0008	0.0162866	-1.77144	293.15	293.15	0	307.413	307.413	0.0699402	0.0698931

815	35.65	11.8536	20.0008	0.016105	-1.87763	293.15	293.15	0	307.246	307.246	0.0699181	0.0698712

816	35.56	11.7612	20.0008	0.0159798	-1.99117	293.15	293.15	0	307.079	307.079	0.0698962	0.0698495

817	35.46	11.6883	20.0008	0.0158813	-2.10832	293.15	293.15	0	306.909	306.909	0.0698752	0.069828

818	35.38	11.6624	20.0008	0.0158465	-2.22744	293.15	293.15	0	306.744	306.744	0.0698544	0.0698069

819	35.29	11.6487	20.0008	0.0158283	-2.34379	293.15	293.15	0	306.586	306.586	0.0698335	0.069786

820	35.2	11.5775	20.0008	0.015732	-2.48296	293.15	293.15	0	306.406	306.406	0.0698128	0.0697647

821	35.11	11.5186	20.0008	0.0156524	-2.61227	293.15	293.15	0	306.243	306.243	0.0697927	0.0697451

822	35.03	11.4481	20.0008	0.0155569	-2.74692	293.15	293.15	0	306.076	306.076	0.0697722	0.0697254

823	34.95	11.3544	20.0008	0.01543	-2.89341	293.15	293.15	0	305.905	305.905	0.0697533	0.0697063

824	34.87	11.2354	20.0008	0.0152687	-3.03801	293.15	293.15	0	305.739	305.739	0.069734	0.0696863

825	34.78	11.1025	20.0008	0.0150885	-3.17513	293.15	293.15	0	305.584	305.584	0.0697141	0.0696669

826	34.71	11.0038	20.0008	0.0149547	-3.33384	293.15	293.15	0	305.411	305.411	0.0696958	0.0696484

827	34.63	10.9495	20.0008	0.0148812	-3.49647	293.15	293.15	0	305.238	305.238	0.0696765	0.0696295

828	34.55	10.905	20.0008	0.0148212	-3.65904	293.15	293.15	0	305.073	305.073	0.0696589	0.0696119

829	34.48	10.8535	20.0008	0.0147515	-3.83095	293.15	293.15	0	304.9	304.9	0.0696404	0.0695939

830	34.4	10.7712	20.0008	0.01464	-4.00077	293.15	293.15	0	304.737	304.737	0.0696229	0.0695763

831	34.32	10.6196	20.0008	0.0144342	-4.16672	293.15	293.15	0	304.579	304.579	0.0696051	0.0695582

832	34.25	10.4745	20.0008	0.0142373	-4.34412	293.15	293.15	0	304.416	304.416	0.0695877	0.069541

833	34.18	10.4077	20.0008	0.0141468	-4.53691	293.15	293.15	0	304.242	304.242	0.0695704	0.0695239

834	34.11	10.3917	20.0008	0.0141254	-4.73195	293.15	293.15	0	304.07	304.07	0.0695534	0.0695064

835	34.03	10.3784	19.9966	0.0141077	-4.92744	293.15	293.15	0	303.906	303.906	0.069537	0.0694896

836	33.97	10.3262	19.9904	0.014037	-5.1255	293.15	293.15	0	303.739	303.739	0.0695206	0.0694739

837	33.9	10.2615	19.9904	0.0139493	-5.32194	293.15	293.15	0	303.579	303.579	0.0695042	0.0694573

838	33.83	10.1397	19.9987	0.0137841	-5.53175	293.15	293.15	0	303.411	303.411	0.0694872	0.0694415

839	33.77	9.97658	20.0008	0.0135625	-5.75629	293.15	293.15	0	303.238	303.238	0.0694725	0.0694263
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RT54-0.25 GNP-0.75 MWCNT.txt
# Name: RT54-0.25 GNP-0.75 MWCNT

# Date: Tue May 21 12:07:50 2024

# Weight: 13.5 mg

Time(s)	Temperature(°C)	Heat flow(mW)	Gas 1(sccm/min)	DSC_RAW(µV)	POWER(%)	TEMP_CJR_FURNACE(K)	TEMP_CJR_SAMPLE(K)	TEMP_FURNACE(K)	TEMP_NOM_FURNACE(K)	TEMP_NOM_SAMPLE(K)	VOLTAGE_REFERENCE(V)	VOLTAGE_SAMPLE(V)

0	29.91	0.209056	20.0008	0.000284533	0.0756808	293.15	293.15	0	303.268	303.268	0.0685574	0.0685133

1	29.93	0.467637	20.0008	0.000636469	0.13537	293.15	293.15	0	303.433	303.433	0.0685617	0.0685185

2	30.02	0.281862	19.9966	0.000383612	0.179563	293.15	293.15	0	303.606	303.606	0.0685799	0.0685388

3	30.14	-0.476208	19.9904	-0.000648093	0.208005	293.15	293.15	0	303.762	303.762	0.0686062	0.0685677

4	30.3	-1.65351	19.9956	-0.00225023	0.23577	293.15	293.15	0	303.943	303.943	0.06864	0.0686043

5	30.46	-3.07087	19.9904	-0.00417887	0.251947	293.15	293.15	0	304.092	304.092	0.068677	0.0686439

6	30.64	-4.57989	19.9904	-0.00623202	0.263097	293.15	293.15	0	304.256	304.256	0.0687172	0.0686862

7	30.83	-6.075	19.9935	-0.00826599	0.269915	293.15	293.15	0	304.43	304.43	0.0687603	0.068731

8	31.02	-7.39974	20.0008	-0.0100679	0.278209	293.15	293.15	0	304.599	304.599	0.0688035	0.0687765

9	31.22	-8.51138	20.0008	-0.0115797	0.282858	293.15	293.15	0	304.759	304.759	0.0688488	0.0688222

10	31.41	-9.37564	20.0029	-0.0127548	0.28405	293.15	293.15	0	304.928	304.928	0.0688933	0.0688681

11	31.59	-10.0928	20.0091	-0.0137296	0.286139	293.15	293.15	0	305.097	305.097	0.0689373	0.0689115

12	31.78	-10.6086	20.0008	-0.0144305	0.287174	293.15	293.15	0	305.273	305.273	0.0689814	0.0689559

13	31.96	-10.9016	19.9998	-0.0148283	0.290935	293.15	293.15	0	305.426	305.426	0.0690243	0.0689989

14	32.15	-11.0263	19.9914	-0.014997	0.291868	293.15	293.15	0	305.601	305.601	0.069068	0.0690434

15	32.33	-11.1198	20.0008	-0.0151232	0.293397	293.15	293.15	0	305.773	305.773	0.0691112	0.0690867

16	32.51	-11.2199	20.0008	-0.0152586	0.293889	293.15	293.15	0	305.939	305.939	0.0691535	0.0691289

17	32.69	-11.2869	20.0008	-0.0153488	0.29657	293.15	293.15	0	306.094	306.094	0.0691955	0.0691719

18	32.87	-11.2739	20.0008	-0.0153303	0.299161	293.15	293.15	0	306.267	306.267	0.0692378	0.0692139

19	33.04	-11.2897	20.0008	-0.015351	0.300123	293.15	293.15	0	306.423	306.423	0.0692794	0.069255

20	33.22	-11.2964	20.0008	-0.0153593	0.300719	293.15	293.15	0	306.597	306.597	0.0693205	0.0692966

21	33.39	-11.2715	20.0008	-0.0153247	0.300755	293.15	293.15	0	306.768	306.768	0.069361	0.0693375

22	33.57	-11.2096	20.0008	-0.0152397	0.308201	293.15	293.15	0	306.934	306.934	0.0694023	0.0693791

23	33.73	-11.1516	20.0008	-0.0151601	0.309615	293.15	293.15	0	307.091	307.091	0.0694414	0.0694183

24	33.9	-11.0875	19.9977	-0.0150721	0.311957	293.15	293.15	0	307.26	307.26	0.0694819	0.0694586

25	34.08	-11.0669	19.9935	-0.0150434	0.317005	293.15	293.15	0	307.438	307.438	0.0695226	0.0694993

26	34.25	-11.0522	20.0008	-0.0150226	0.318686	293.15	293.15	0	307.598	307.598	0.0695629	0.0695396

27	34.41	-10.9808	20.0008	-0.0149248	0.321746	293.15	293.15	0	307.767	307.767	0.0696028	0.0695789

28	34.58	-10.8996	19.9987	-0.0148137	0.324095	293.15	293.15	0	307.935	307.935	0.0696419	0.0696189

29	34.75	-10.8245	19.9977	-0.0147108	0.325852	293.15	293.15	0	308.105	308.105	0.0696817	0.0696591

30	34.92	-10.7741	20.0008	-0.0146416	0.330947	293.15	293.15	0	308.272	308.272	0.0697218	0.0696992

31	35.09	-10.7653	20.0008	-0.0146289	0.334313	293.15	293.15	0	308.434	308.434	0.0697614	0.069739

32	35.25	-10.7689	20.0008	-0.014633	0.33532	293.15	293.15	0	308.598	308.598	0.0698012	0.0697782

33	35.42	-10.7239	20.0008	-0.0145712	0.340704	293.15	293.15	0	308.771	308.771	0.0698402	0.0698174

34	35.59	-10.6902	20.0008	-0.0145246	0.343959	293.15	293.15	0	308.929	308.929	0.0698794	0.0698572

35	35.76	-10.698	20.0008	-0.0145345	0.345147	293.15	293.15	0	309.093	309.093	0.0699199	0.0698976

36	35.92	-10.7011	20.0008	-0.014538	0.351107	293.15	293.15	0	309.266	309.266	0.069958	0.0699361

37	36.09	-10.7214	19.9956	-0.0145647	0.350332	293.15	293.15	0	309.439	309.439	0.0699984	0.0699769

38	36.26	-10.7456	20.0008	-0.0145969	0.354416	293.15	293.15	0	309.602	309.602	0.070037	0.0700157

39	36.43	-10.7537	20.0008	-0.0146071	0.357644	293.15	293.15	0	309.76	309.76	0.0700776	0.0700564

40	36.59	-10.7849	19.9956	-0.0146488	0.361181	293.15	293.15	0	309.933	309.933	0.0701165	0.0700951

41	36.76	-10.8122	20.0008	-0.0146851	0.363251	293.15	293.15	0	310.105	310.105	0.070156	0.0701352

42	36.93	-10.8408	20.0008	-0.0147231	0.366572	293.15	293.15	0	310.272	310.272	0.0701956	0.0701755

43	37.1	-10.8822	19.9977	-0.0147786	0.371598	293.15	293.15	0	310.432	310.432	0.0702347	0.0702141

44	37.27	-10.903	19.9935	-0.0148061	0.37485	293.15	293.15	0	310.605	310.605	0.070274	0.0702539

45	37.43	-10.9105	20.0008	-0.0148156	0.37849	293.15	293.15	0	310.766	310.766	0.0703134	0.0702932

46	37.6	-10.913	20.0008	-0.0148182	0.379909	293.15	293.15	0	310.931	310.931	0.070353	0.0703326

47	37.77	-10.8959	20.0008	-0.0147943	0.382609	293.15	293.15	0	311.089	311.089	0.0703924	0.0703724

48	37.93	-10.8907	20.0019	-0.0147864	0.387866	293.15	293.15	0	311.26	311.26	0.0704314	0.0704114

49	38.11	-10.8261	20.005	-0.0146979	0.388768	293.15	293.15	0	311.433	311.433	0.0704718	0.070452

50	38.27	-10.7633	20.0008	-0.0146119	0.393314	293.15	293.15	0	311.59	311.59	0.0705107	0.0704909

51	38.44	-10.7801	20.0008	-0.0146341	0.396642	293.15	293.15	0	311.763	311.763	0.0705497	0.0705301

52	38.61	-10.8172	19.9956	-0.0146836	0.402219	293.15	293.15	0	311.927	311.927	0.0705893	0.0705701

53	38.77	-10.813	19.9904	-0.0146772	0.404962	293.15	293.15	0	312.1	312.1	0.0706288	0.0706096

54	38.94	-10.7782	20.0008	-0.0146292	0.407362	293.15	293.15	0	312.265	312.265	0.0706677	0.0706493

55	39.11	-10.7511	20.0008	-0.0145917	0.408863	293.15	293.15	0	312.43	312.43	0.0707071	0.0706885

56	39.27	-10.7402	20.0008	-0.0145761	0.411263	293.15	293.15	0	312.602	312.602	0.070746	0.0707276

57	39.44	-10.7594	19.9966	-0.0146015	0.41817	293.15	293.15	0	312.767	312.767	0.0707852	0.0707668

58	39.6	-10.866	19.9935	-0.0147454	0.424345	293.15	293.15	0	312.939	312.939	0.0708241	0.070806

59	39.78	-10.9328	20.0008	-0.0148352	0.423372	293.15	293.15	0	313.098	313.098	0.0708643	0.070847

60	39.94	-10.9562	20.0008	-0.0148663	0.426719	293.15	293.15	0	313.276	313.276	0.070904	0.0708863

61	40.11	-11.0578	20.0008	-0.0150034	0.430954	293.15	293.15	0	313.428	313.428	0.0709428	0.0709254

62	40.28	-11.3099	20.0008	-0.0153446	0.435077	293.15	293.15	0	313.601	313.601	0.0709822	0.0709661

63	40.45	-11.5339	20.0008	-0.0156478	0.437955	293.15	293.15	0	313.765	313.765	0.0710211	0.0710046

64	40.62	-11.6387	20.0008	-0.0157891	0.439669	293.15	293.15	0	313.923	313.923	0.0710611	0.0710452

65	40.78	-11.6733	20.0008	-0.0158352	0.444019	293.15	293.15	0	314.094	314.094	0.0711011	0.0710845

66	40.95	-11.6918	20.0008	-0.0158594	0.446534	293.15	293.15	0	314.26	314.26	0.0711398	0.0711237

67	41.12	-11.6964	20.0008	-0.015865	0.447936	293.15	293.15	0	314.424	314.424	0.0711791	0.071163

68	41.28	-11.7381	20.0008	-0.0159207	0.454616	293.15	293.15	0	314.607	314.607	0.0712176	0.0712022

69	41.45	-11.731	20.0008	-0.0159103	0.457131	293.15	293.15	0	314.771	314.771	0.0712567	0.0712411

70	41.62	-11.7039	20.0008	-0.0158727	0.458269	293.15	293.15	0	314.937	314.937	0.0712972	0.0712817

71	41.79	-11.7058	20.0008	-0.0158744	0.464554	293.15	293.15	0	315.099	315.099	0.0713359	0.0713206

72	41.95	-11.6967	20.0008	-0.0158613	0.466524	293.15	293.15	0	315.264	315.264	0.071375	0.07136

73	42.12	-11.641	20.0008	-0.0157849	0.471611	293.15	293.15	0	315.438	315.438	0.0714144	0.0713992

74	42.28	-11.6227	20.0008	-0.0157594	0.474041	293.15	293.15	0	315.6	315.6	0.0714526	0.0714378

75	42.45	-11.677	19.9977	-0.0158321	0.480229	293.15	293.15	0	315.768	315.768	0.0714922	0.0714782

76	42.62	-11.7279	19.9987	-0.0159004	0.483572	293.15	293.15	0	315.938	315.938	0.0715321	0.071518

77	42.79	-11.7773	20.0039	-0.0159665	0.484976	293.15	293.15	0	316.106	316.106	0.0715723	0.0715574

78	42.95	-11.7512	20.0091	-0.0159304	0.486839	293.15	293.15	0	316.271	316.271	0.0716104	0.0715958

79	43.12	-11.673	20.0008	-0.0158235	0.493622	293.15	293.15	0	316.429	316.429	0.0716499	0.0716361

80	43.29	-11.6032	19.9987	-0.015728	0.496954	293.15	293.15	0	316.6	316.6	0.0716893	0.0716751

81	43.45	-11.6333	19.9914	-0.0157681	0.498397	293.15	293.15	0	316.765	316.765	0.0717285	0.0717141

82	43.62	-11.6772	20.0008	-0.0158268	0.500214	293.15	293.15	0	316.922	316.922	0.0717682	0.0717543

83	43.79	-11.7603	20.0008	-0.0159387	0.504493	293.15	293.15	0	317.093	317.093	0.0718067	0.0717934

84	43.96	-11.7911	19.9998	-0.0159796	0.511172	293.15	293.15	0	317.268	317.268	0.0718459	0.0718325

85	44.13	-11.777	19.9966	-0.0159596	0.51567	293.15	293.15	0	317.439	317.439	0.0718853	0.0718722

86	44.29	-11.7629	20.0008	-0.0159397	0.518702	293.15	293.15	0	317.606	317.606	0.0719232	0.0719106

87	44.46	-11.7385	19.9904	-0.0159059	0.522782	293.15	293.15	0	317.761	317.761	0.0719635	0.0719509

88	44.63	-11.8038	20.0008	-0.0159935	0.524754	293.15	293.15	0	317.934	317.934	0.0720034	0.0719909

89	44.8	-11.7884	20.0008	-0.0159718	0.528553	293.15	293.15	0	318.108	318.108	0.0720423	0.0720303

90	44.96	-11.7193	20.0008	-0.0158774	0.530636	293.15	293.15	0	318.273	318.273	0.072081	0.0720683

91	45.13	-11.7066	20.0008	-0.0158595	0.533549	293.15	293.15	0	318.435	318.435	0.07212	0.0721084

92	45.3	-11.7255	20.0008	-0.0158842	0.538926	293.15	293.15	0	318.6	318.6	0.0721599	0.072148

93	45.47	-11.8443	20.0008	-0.0160442	0.539173	293.15	293.15	0	318.757	318.757	0.0722002	0.0721891

94	45.64	-11.975	20.0008	-0.0162205	0.542221	293.15	293.15	0	318.927	318.927	0.0722394	0.0722287

95	45.8	-11.9701	19.9977	-0.016213	0.549808	293.15	293.15	0	319.104	319.104	0.0722783	0.0722671

96	45.96	-11.9515	19.9925	-0.016187	0.55378	293.15	293.15	0	319.264	319.264	0.0723172	0.0723054

97	46.13	-11.9818	20.0008	-0.0162272	0.554916	293.15	293.15	0	319.434	319.434	0.0723573	0.072345

98	46.3	-12.0049	20.0008	-0.0162577	0.558702	293.15	293.15	0	319.602	319.602	0.0723955	0.072384

99	46.46	-11.9755	20.0008	-0.0162171	0.562353	293.15	293.15	0	319.771	319.771	0.0724341	0.0724232

100	46.64	-11.9854	20.0008	-0.0162296	0.567762	293.15	293.15	0	319.939	319.939	0.0724738	0.0724634

101	46.8	-12.0498	20.0008	-0.016316	0.570655	293.15	293.15	0	320.101	320.101	0.0725128	0.0725021

102	46.97	-12.0605	20.0008	-0.0163297	0.573512	293.15	293.15	0	320.267	320.267	0.0725524	0.0725421

103	47.14	-12.0164	20.0008	-0.0162691	0.577288	293.15	293.15	0	320.422	320.422	0.0725914	0.0725813

104	47.3	-11.97	20.0008	-0.0162055	0.578627	293.15	293.15	0	320.604	320.604	0.0726311	0.0726209

105	47.47	-11.9562	20.0008	-0.016186	0.587667	293.15	293.15	0	320.768	320.768	0.0726694	0.0726599

106	47.64	-11.9538	20.0008	-0.0161819	0.586101	293.15	293.15	0	320.941	320.941	0.0727096	0.0726988

107	47.8	-11.9369	19.9956	-0.0161582	0.59329	293.15	293.15	0	321.098	321.098	0.0727471	0.0727378

108	47.97	-11.8674	20.0008	-0.0160633	0.595924	293.15	293.15	0	321.264	321.264	0.0727869	0.072777

109	48.14	-11.8467	20.0008	-0.0160345	0.596826	293.15	293.15	0	321.424	321.424	0.0728273	0.0728175

110	48.31	-11.8639	19.9977	-0.0160569	0.603871	293.15	293.15	0	321.602	321.602	0.0728655	0.0728568

111	48.47	-11.8633	19.9967	-0.0160554	0.607	293.15	293.15	0	321.766	321.766	0.0729044	0.0728955

112	48.64	-11.8969	20.0091	-0.0160999	0.609817	293.15	293.15	0	321.927	321.927	0.0729437	0.0729348

113	48.81	-11.9671	20.0008	-0.0161942	0.612229	293.15	293.15	0	322.096	322.096	0.0729832	0.0729746

114	48.98	-12.0149	20.0008	-0.016258	0.617924	293.15	293.15	0	322.263	322.263	0.0730227	0.0730142

115	49.14	-12.0327	20.0008	-0.0162813	0.61984	293.15	293.15	0	322.441	322.441	0.0730621	0.0730535

116	49.31	-12.0218	20.0008	-0.0162657	0.621756	293.15	293.15	0	322.6	322.6	0.0731014	0.0730932

117	49.48	-12.0354	19.9998	-0.0162833	0.624599	293.15	293.15	0	322.763	322.763	0.0731409	0.0731328

118	49.64	-11.9715	19.9966	-0.0161959	0.630994	293.15	293.15	0	322.937	322.937	0.0731802	0.0731712

119	49.81	-11.8353	20.0008	-0.0160109	0.634074	293.15	293.15	0	323.109	323.109	0.0732185	0.0732103

120	49.97	-11.7467	20.0008	-0.0158902	0.63866	293.15	293.15	0	323.274	323.274	0.0732568	0.0732489

121	50.14	-11.785	20.0008	-0.0159412	0.643657	293.15	293.15	0	323.429	323.429	0.0732954	0.073288

122	50.31	-11.8541	20.0008	-0.0160339	0.645615	293.15	293.15	0	323.603	323.603	0.0733363	0.0733285

123	50.48	-11.9446	20.0008	-0.0161556	0.649765	293.15	293.15	0	323.758	323.758	0.0733743	0.0733671

124	50.65	-11.9663	20.0008	-0.016184	0.65364	293.15	293.15	0	323.933	323.933	0.0734137	0.0734065

125	50.82	-11.9275	20.0008	-0.0161307	0.655782	293.15	293.15	0	324.096	324.096	0.0734534	0.0734467

126	50.98	-11.8444	20.0008	-0.0160176	0.659269	293.15	293.15	0	324.268	324.268	0.0734912	0.0734846

127	51.15	-11.905	19.9977	-0.0160986	0.662961	293.15	293.15	0	324.427	324.427	0.073531	0.0735252

128	51.32	-11.9716	19.9935	-0.0161879	0.669297	293.15	293.15	0	324.597	324.597	0.0735697	0.073564

129	51.48	-12.0211	20.0008	-0.016254	0.67253	293.15	293.15	0	324.765	324.765	0.0736091	0.0736026

130	51.65	-12.0824	19.9987	-0.0163361	0.676456	293.15	293.15	0	324.934	324.934	0.0736486	0.0736431

131	51.82	-12.0974	19.9925	-0.0163555	0.679807	293.15	293.15	0	325.094	325.094	0.0736876	0.0736825

132	51.99	-12.1153	20.0008	-0.0163788	0.686394	293.15	293.15	0	325.267	325.267	0.073726	0.0737213

133	52.15	-12.1404	20.0008	-0.016412	0.688302	293.15	293.15	0	325.431	325.431	0.0737657	0.073761

134	52.32	-12.1618	20.0008	-0.01644	0.689148	293.15	293.15	0	325.599	325.599	0.0738057	0.0738002

135	52.49	-12.1792	20.0071	-0.0164628	0.69303	293.15	293.15	0	325.761	325.761	0.0738445	0.0738391

136	52.65	-12.1792	20.0102	-0.016462	0.69855	293.15	293.15	0	325.927	325.927	0.0738833	0.0738784

137	52.82	-12.1679	20.0008	-0.0164458	0.704453	293.15	293.15	0	326.108	326.108	0.0739215	0.0739176

138	52.99	-12.1219	20.0008	-0.0163828	0.706908	293.15	293.15	0	326.264	326.264	0.0739609	0.0739567

139	53.15	-12.1098	20.0008	-0.0163657	0.709193	293.15	293.15	0	326.428	326.428	0.0740001	0.0739956

140	53.32	-12.1181	20.0008	-0.016376	0.712996	293.15	293.15	0	326.602	326.602	0.0740406	0.0740357

141	53.49	-12.1443	20.0008	-0.0164106	0.718463	293.15	293.15	0	326.775	326.775	0.0740789	0.0740748

142	53.66	-12.1577	20.0008	-0.0164279	0.720774	293.15	293.15	0	326.939	326.939	0.0741178	0.0741139

143	53.83	-12.0818	19.9956	-0.0163245	0.722143	293.15	293.15	0	327.095	327.095	0.0741577	0.0741535

144	53.99	-12.0837	19.9977	-0.0163262	0.726596	293.15	293.15	0	327.267	327.267	0.0741962	0.074192

145	54.16	-12.1298	19.9935	-0.0163876	0.735376	293.15	293.15	0	327.435	327.435	0.074235	0.0742315

146	54.32	-12.1859	20.0008	-0.0164626	0.741271	293.15	293.15	0	327.604	327.604	0.0742724	0.07427

147	54.49	-12.202	20.0008	-0.0164836	0.742469	293.15	293.15	0	327.756	327.756	0.0743125	0.0743102

148	54.66	-12.2402	20.0008	-0.0165344	0.743242	293.15	293.15	0	327.932	327.932	0.0743522	0.0743492

149	54.83	-12.2953	20.0008	-0.0166079	0.750176	293.15	293.15	0	328.102	328.102	0.0743917	0.0743892

150	55	-12.3404	20.0008	-0.016668	0.754734	293.15	293.15	0	328.275	328.275	0.0744299	0.0744282

151	55.16	-12.3541	19.9946	-0.0166857	0.756104	293.15	293.15	0	328.424	328.424	0.074469	0.0744673

152	55.33	-12.365	19.9966	-0.0166995	0.759941	293.15	293.15	0	328.595	328.595	0.0745087	0.0745068

153	55.5	-12.3692	20.0008	-0.0167044	0.765933	293.15	293.15	0	328.769	328.769	0.0745473	0.0745452

154	55.67	-12.3853	20.0008	-0.0167253	0.767128	293.15	293.15	0	328.935	328.935	0.0745871	0.0745855

155	55.83	-12.4244	20.0008	-0.0167771	0.772567	293.15	293.15	0	329.099	329.099	0.0746252	0.074624

156	56	-12.4845	20.0008	-0.0168575	0.777285	293.15	293.15	0	329.263	329.263	0.074664	0.0746631

157	56.17	-12.5427	20.0008	-0.0169353	0.781987	293.15	293.15	0	329.436	329.436	0.0747033	0.0747022

158	56.33	-12.6341	20.0008	-0.0170578	0.784806	293.15	293.15	0	329.601	329.601	0.0747427	0.0747418

159	56.5	-12.7513	20.0008	-0.0172152	0.78851	293.15	293.15	0	329.766	329.766	0.0747812	0.0747808

160	56.67	-12.8645	20.0008	-0.017367	0.793855	293.15	293.15	0	329.937	329.937	0.0748203	0.0748203

161	56.83	-12.9929	20.0008	-0.0175396	0.795865	293.15	293.15	0	330.087	330.087	0.0748585	0.0748589

162	57	-13.1772	20.0008	-0.0177874	0.80384	293.15	293.15	0	330.265	330.265	0.0748977	0.0748987

163	57.17	-13.3526	19.9987	-0.0180232	0.808853	293.15	293.15	0	330.426	330.426	0.0749364	0.0749376

164	57.34	-13.4835	19.9925	-0.018199	0.812382	293.15	293.15	0	330.594	330.594	0.0749758	0.074977

165	57.5	-13.5876	20.0008	-0.0183386	0.817518	293.15	293.15	0	330.763	330.763	0.0750132	0.075015

166	57.67	-13.7304	20.0008	-0.0185304	0.821578	293.15	293.15	0	330.94	330.94	0.0750526	0.0750541

167	57.84	-13.8992	20.0008	-0.0187573	0.828712	293.15	293.15	0	331.111	331.111	0.0750915	0.0750937

168	58	-14.1177	20.0008	-0.0190512	0.833973	293.15	293.15	0	331.268	331.268	0.0751295	0.0751329

169	58.18	-14.4712	19.9946	-0.0195271	0.83636	293.15	293.15	0	331.44	331.44	0.0751686	0.0751731

170	58.34	-14.9142	19.9904	-0.020124	0.844195	293.15	293.15	0	331.617	331.617	0.0752066	0.0752115

171	58.5	-15.4329	19.9998	-0.0208228	0.852966	293.15	293.15	0	331.763	331.763	0.0752432	0.0752498

172	58.67	-16.1443	20.0008	-0.0217816	0.862642	293.15	293.15	0	331.937	331.937	0.0752809	0.0752891

173	58.83	-16.9508	20.0008	-0.0228685	0.870787	293.15	293.15	0	332.099	332.099	0.0753176	0.075327

174	59	-17.909	20.0008	-0.0241601	0.880907	293.15	293.15	0	332.261	332.261	0.0753545	0.0753656

175	59.16	-19.0568	19.9977	-0.0257073	0.896213	293.15	293.15	0	332.43	332.43	0.0753898	0.0754035

176	59.32	-20.472	19.9935	-0.027615	0.910182	293.15	293.15	0	332.599	332.599	0.0754253	0.0754414

177	59.49	-22.3244	19.9987	-0.0301122	0.925358	293.15	293.15	0	332.759	332.759	0.0754607	0.0754805

178	59.65	-24.5814	19.9925	-0.0331549	0.941267	293.15	293.15	0	332.927	332.927	0.0754953	0.0755188

179	59.81	-27.198	20.0008	-0.0366823	0.962214	293.15	293.15	0	333.096	333.096	0.0755275	0.0755565

180	59.98	-30.139	19.9987	-0.0406468	0.984337	293.15	293.15	0	333.27	333.27	0.0755609	0.0755951

181	60.14	-33.374	19.9914	-0.0450075	1.00533	293.15	293.15	0	333.419	333.419	0.0755942	0.0756333

182	60.31	-36.9351	19.9946	-0.0498073	1.02855	293.15	293.15	0	333.591	333.591	0.0756277	0.0756725

183	60.47	-40.5631	19.9914	-0.054697	1.05244	293.15	293.15	0	333.764	333.764	0.0756613	0.0757113

184	60.65	-44.4033	20.0008	-0.0598722	1.07479	293.15	293.15	0	333.93	333.93	0.0756962	0.0757518

185	60.82	-48.1426	20.0008	-0.0649108	1.10277	293.15	293.15	0	334.11	334.11	0.0757315	0.0757922

186	60.99	-51.8535	20.0008	-0.0699105	1.12116	293.15	293.15	0	334.267	334.267	0.0757671	0.0758331

187	61.18	-55.5599	20.0008	-0.0749034	1.14009	293.15	293.15	0	334.432	334.432	0.0758045	0.0758759

188	61.36	-59.3734	20.0008	-0.0800403	1.16282	293.15	293.15	0	334.604	334.604	0.0758413	0.0759181

189	61.54	-63.2443	20.0008	-0.0852539	1.18129	293.15	293.15	0	334.769	334.769	0.0758791	0.0759603

190	61.72	-67.1198	20.0008	-0.090473	1.20476	293.15	293.15	0	334.934	334.934	0.075917	0.0760038

191	61.9	-70.7017	20.0008	-0.0952959	1.22116	293.15	293.15	0	335.096	335.096	0.0759549	0.0760459

192	62.1	-74.1587	20.0008	-0.0999496	1.23961	293.15	293.15	0	335.262	335.262	0.0759949	0.076091

193	62.29	-77.2527	20.0008	-0.104114	1.25403	293.15	293.15	0	335.435	335.435	0.0760361	0.0761355

194	62.48	-80.0715	20.0008	-0.107906	1.26679	293.15	293.15	0	335.598	335.598	0.0760782	0.0761805

195	62.67	-82.5224	20.0008	-0.111203	1.27896	293.15	293.15	0	335.765	335.765	0.0761207	0.0762257

196	62.87	-84.5914	19.9977	-0.113984	1.2863	293.15	293.15	0	335.936	335.936	0.0761643	0.0762711

197	63.06	-86.2481	19.9925	-0.11621	1.29341	293.15	293.15	0	336.086	336.086	0.0762078	0.0763162

198	63.26	-87.7511	20.0008	-0.118228	1.30159	293.15	293.15	0	336.263	336.263	0.0762512	0.0763619

199	63.45	-89.0663	20.0008	-0.119993	1.30417	293.15	293.15	0	336.432	336.432	0.076295	0.0764067

200	63.64	-89.8417	19.9987	-0.12103	1.30111	293.15	293.15	0	336.606	336.606	0.0763418	0.0764524

201	63.83	-90.0158	19.9914	-0.121258	1.29837	293.15	293.15	0	336.755	336.755	0.0763884	0.0764971

202	64.03	-89.7102	20.0008	-0.120839	1.29877	293.15	293.15	0	336.926	336.926	0.0764341	0.0765424

203	64.22	-88.9028	20.0008	-0.119745	1.29108	293.15	293.15	0	337.1	337.1	0.076481	0.076587

204	64.42	-87.698	20.0008	-0.118115	1.28108	293.15	293.15	0	337.266	337.266	0.0765293	0.076633

205	64.61	-86.2181	20.0008	-0.116115	1.27062	293.15	293.15	0	337.431	337.431	0.0765772	0.0766779

206	64.79	-84.4033	20.0008	-0.113664	1.26362	293.15	293.15	0	337.594	337.594	0.0766232	0.076721

207	64.98	-82.1447	20.0008	-0.110617	1.24871	293.15	293.15	0	337.767	337.767	0.0766711	0.0767646

208	65.16	-79.3927	20.0008	-0.106905	1.23214	293.15	293.15	0	337.94	337.94	0.0767182	0.0768073

209	65.34	-76.1877	20.0008	-0.102584	1.21677	293.15	293.15	0	338.088	338.088	0.0767649	0.0768485

210	65.52	-72.7303	20.0008	-0.0979232	1.19683	293.15	293.15	0	338.268	338.268	0.0768118	0.0768905

211	65.69	-69.3383	20.0008	-0.0933513	1.18602	293.15	293.15	0	338.434	338.434	0.0768566	0.0769314

212	65.86	-66.2298	20.0008	-0.0891618	1.17483	293.15	293.15	0	338.606	338.606	0.0768984	0.0769698

213	66.02	-63.2948	20.0008	-0.0852064	1.16756	293.15	293.15	0	338.765	338.765	0.0769397	0.0770075

214	66.17	-60.3887	20.0008	-0.0812904	1.16049	293.15	293.15	0	338.938	338.938	0.0769795	0.077044

215	66.33	-57.5222	20.0008	-0.077428	1.1512	293.15	293.15	0	339.107	339.107	0.0770198	0.077081

216	66.49	-54.8164	19.9946	-0.0737824	1.1421	293.15	293.15	0	339.266	339.266	0.0770593	0.0771169

217	66.64	-52.1852	20.0008	-0.0702375	1.13396	293.15	293.15	0	339.431	339.431	0.0770987	0.0771533

218	66.79	-49.6041	20.0008	-0.0667605	1.12701	293.15	293.15	0	339.599	339.599	0.0771369	0.0771882

219	66.94	-47.1301	19.9998	-0.063428	1.12528	293.15	293.15	0	339.759	339.759	0.077175	0.0772236

220	67.1	-44.7861	19.9914	-0.0602706	1.11864	293.15	293.15	0	339.927	339.927	0.0772131	0.077259

221	67.24	-42.6704	20.0008	-0.057421	1.11728	293.15	293.15	0	340.098	340.098	0.0772489	0.0772925

222	67.39	-40.7016	20.0008	-0.054769	1.1131	293.15	293.15	0	340.265	340.265	0.0772866	0.0773281

223	67.54	-38.9156	20.0008	-0.0523635	1.11416	293.15	293.15	0	340.419	340.419	0.0773227	0.0773623

224	67.68	-37.2011	20.0008	-0.0500542	1.11517	293.15	293.15	0	340.601	340.601	0.0773585	0.0773965

225	67.84	-35.4787	20.0008	-0.0477345	1.11018	293.15	293.15	0	340.765	340.765	0.077397	0.0774319

226	67.99	-33.7664	20.0008	-0.0454287	1.10493	293.15	293.15	0	340.929	340.929	0.0774353	0.0774681

227	68.14	-31.9841	20.0008	-0.0430288	1.10049	293.15	293.15	0	341.105	341.105	0.0774734	0.0775038

228	68.3	-30.1018	20.0008	-0.0404946	1.09629	293.15	293.15	0	341.276	341.276	0.0775125	0.0775396

229	68.45	-28.0924	20.0008	-0.0377896	1.09323	293.15	293.15	0	341.426	341.426	0.0775516	0.0775759

230	68.61	-25.8622	20.0008	-0.034788	1.08851	293.15	293.15	0	341.604	341.604	0.0775914	0.0776132

231	68.77	-23.4829	20.0008	-0.031586	1.08081	293.15	293.15	0	341.773	341.773	0.0776319	0.07765

232	68.93	-21.2075	20.0008	-0.028524	1.07457	293.15	293.15	0	341.938	341.938	0.0776712	0.0776872

233	69.08	-19.243	20.0008	-0.0258806	1.07551	293.15	293.15	0	342.093	342.093	0.0777081	0.0777225

234	69.24	-17.5308	20.0008	-0.0235768	1.07294	293.15	293.15	0	342.26	342.26	0.0777459	0.0777588

235	69.39	-16.1138	20.0008	-0.02167	1.07023	293.15	293.15	0	342.43	342.43	0.0777834	0.0777943

236	69.54	-14.924	20.0008	-0.0200691	1.07218	293.15	293.15	0	342.607	342.607	0.0778185	0.0778285

237	69.69	-13.893	20.0008	-0.0186818	1.07607	293.15	293.15	0	342.76	342.76	0.0778537	0.0778634

238	69.83	-13.0714	20.0008	-0.0175762	1.08293	293.15	293.15	0	342.933	342.933	0.0778884	0.0778974

239	69.98	-12.4608	20.0008	-0.0167545	1.08567	293.15	293.15	0	343.099	343.099	0.0779238	0.0779324

240	70.13	-12.0414	20.0008	-0.0161898	1.09525	293.15	293.15	0	343.271	343.271	0.0779586	0.0779673

241	70.28	-11.7727	20.0008	-0.0158278	1.10383	293.15	293.15	0	343.427	343.427	0.0779935	0.0780024

242	70.44	-11.6276	20.0008	-0.0156319	1.10777	293.15	293.15	0	343.6	343.6	0.0780295	0.0780384

243	70.59	-11.555	20.0008	-0.0155336	1.11183	293.15	293.15	0	343.773	343.773	0.0780657	0.0780748

244	70.75	-11.4938	20.0008	-0.0154506	1.11775	293.15	293.15	0	343.928	343.928	0.078102	0.0781118

245	70.91	-11.4244	20.0008	-0.0153566	1.12285	293.15	293.15	0	344.094	344.094	0.0781389	0.0781486

246	71.07	-11.4055	20.0008	-0.0153305	1.13167	293.15	293.15	0	344.266	344.266	0.0781752	0.0781851

247	71.23	-11.4436	20.0008	-0.015381	1.13675	293.15	293.15	0	344.441	344.441	0.0782125	0.0782232

248	71.39	-11.4817	20.0008	-0.0154314	1.14525	293.15	293.15	0	344.604	344.604	0.0782498	0.0782612

249	71.55	-11.5661	20.0008	-0.0155441	1.14821	293.15	293.15	0	344.762	344.762	0.0782879	0.0782986

250	71.72	-11.661	20.0008	-0.0156708	1.15481	293.15	293.15	0	344.94	344.94	0.0783266	0.0783373

251	71.89	-11.7555	20.0008	-0.015797	1.15981	293.15	293.15	0	345.108	345.108	0.0783644	0.0783759

252	72.05	-11.8495	20.0008	-0.0159225	1.16194	293.15	293.15	0	345.263	345.263	0.0784031	0.0784141

253	72.21	-11.9321	20.0008	-0.0160328	1.16599	293.15	293.15	0	345.432	345.432	0.0784407	0.0784523

254	72.38	-11.9798	20.0008	-0.016096	1.1745	293.15	293.15	0	345.602	345.602	0.0784797	0.0784919

255	72.55	-11.9914	20.0008	-0.0161109	1.17809	293.15	293.15	0	345.758	345.758	0.078518	0.0785303

256	72.71	-11.9784	20.0008	-0.0160925	1.18177	293.15	293.15	0	345.924	345.924	0.0785564	0.0785684

257	72.88	-11.9475	20.0008	-0.0160502	1.18724	293.15	293.15	0	346.095	346.095	0.0785948	0.0786076

258	73.05	-11.9408	20.0008	-0.0160404	1.1937	293.15	293.15	0	346.271	346.271	0.0786341	0.0786472

259	73.22	-11.9946	20.0008	-0.0161118	1.19552	293.15	293.15	0	346.426	346.426	0.0786727	0.0786856

260	73.38	-12.0993	20.0008	-0.0162517	1.20207	293.15	293.15	0	346.599	346.599	0.0787114	0.0787246

261	73.55	-12.1623	20.0008	-0.0163355	1.20459	293.15	293.15	0	346.772	346.772	0.0787502	0.0787634

262	73.72	-12.2257	20.0008	-0.0164198	1.20815	293.15	293.15	0	346.936	346.936	0.0787889	0.0788019

263	73.88	-12.2237	20.0008	-0.0164163	1.21544	293.15	293.15	0	347.093	347.093	0.0788276	0.0788409

264	74.05	-12.1667	20.0008	-0.016339	1.21839	293.15	293.15	0	347.273	347.273	0.0788663	0.0788798

265	74.22	-12.0979	20.0008	-0.0162457	1.22229	293.15	293.15	0	347.439	347.439	0.0789056	0.0789191

266	74.38	-12.1081	20.0008	-0.0162586	1.22661	293.15	293.15	0	347.594	347.594	0.0789433	0.0789575

267	74.55	-12.172	20.0008	-0.0163435	1.23493	293.15	293.15	0	347.766	347.766	0.0789822	0.0789966

268	74.72	-12.2672	20.0008	-0.0164706	1.24136	293.15	293.15	0	347.935	347.935	0.0790207	0.0790353

269	74.89	-12.329	20.0008	-0.0165528	1.24289	293.15	293.15	0	348.094	348.094	0.07906	0.0790747

270	75.06	-12.3584	20.0008	-0.0165913	1.24566	293.15	293.15	0	348.263	348.263	0.0790996	0.0791144

271	75.22	-12.3459	20.0008	-0.0165737	1.25068	293.15	293.15	0	348.437	348.437	0.0791379	0.079153

272	75.39	-12.2909	19.9987	-0.0164991	1.25653	293.15	293.15	0	348.604	348.604	0.0791765	0.0791917

273	75.56	-12.2634	19.9914	-0.0164613	1.25836	293.15	293.15	0	348.757	348.757	0.0792153	0.079231

274	75.73	-12.2764	20.0008	-0.0164779	1.2634	293.15	293.15	0	348.93	348.93	0.0792544	0.0792698

275	75.9	-12.2668	20.0008	-0.0164642	1.2695	293.15	293.15	0	349.096	349.096	0.0792937	0.0793096

276	76.06	-12.2327	20.0008	-0.0164176	1.27499	293.15	293.15	0	349.269	349.269	0.0793314	0.0793476

277	76.23	-12.108	20.0008	-0.0162495	1.2776	293.15	293.15	0	349.424	349.424	0.0793707	0.0793871

278	76.4	-12.0739	20.0008	-0.0162029	1.28144	293.15	293.15	0	349.598	349.598	0.0794097	0.079426

279	76.57	-12.0339	20.0008	-0.0161484	1.28522	293.15	293.15	0	349.771	349.771	0.0794486	0.0794655

280	76.73	-12.0392	19.9956	-0.0161547	1.29044	293.15	293.15	0	349.935	349.935	0.0794874	0.0795041

281	76.9	-12.0542	20.0008	-0.016174	1.29559	293.15	293.15	0	350.092	350.092	0.079526	0.0795428

282	77.07	-12.0527	20.0008	-0.0161711	1.29795	293.15	293.15	0	350.263	350.263	0.0795652	0.0795817

283	77.23	-12.0167	20.0008	-0.0161221	1.30334	293.15	293.15	0	350.438	350.438	0.0796032	0.0796205

284	77.4	-11.9894	20.0008	-0.0160845	1.30817	293.15	293.15	0	350.6	350.6	0.0796424	0.0796601

285	77.57	-11.9921	20.0008	-0.0160874	1.31575	293.15	293.15	0	350.768	350.768	0.0796809	0.079698

286	77.73	-11.9927	20.0008	-0.0160873	1.31974	293.15	293.15	0	350.928	350.928	0.0797187	0.0797357

287	77.9	-12.0316	20.0008	-0.0161388	1.32445	293.15	293.15	0	351.098	351.098	0.0797567	0.0797747

288	78.07	-12.0805	20.0008	-0.0162036	1.3261	293.15	293.15	0	351.266	351.266	0.0797961	0.0798143

289	78.24	-12.0863	20.0008	-0.0162105	1.33311	293.15	293.15	0	351.435	351.435	0.0798354	0.0798534

290	78.4	-12.0676	20.0008	-0.0161846	1.33592	293.15	293.15	0	351.594	351.594	0.0798744	0.0798923

291	78.57	-11.9888	20.0071	-0.0160781	1.34114	293.15	293.15	0	351.765	351.765	0.0799126	0.0799309

292	78.74	-11.9072	20.0112	-0.0159678	1.34532	293.15	293.15	0	351.932	351.932	0.079951	0.0799694

293	78.9	-11.8696	20.0008	-0.0159167	1.34914	293.15	293.15	0	352.095	352.095	0.0799897	0.0800078

294	79.07	-11.8898	20.0008	-0.0159429	1.35608	293.15	293.15	0	352.269	352.269	0.0800292	0.0800475

295	79.24	-11.8716	20.0008	-0.0159177	1.35951	293.15	293.15	0	352.432	352.432	0.0800681	0.0800861

296	79.4	-11.8719	19.9946	-0.0159173	1.36323	293.15	293.15	0	352.605	352.605	0.0801058	0.0801247

297	79.57	-11.9576	20.0008	-0.0160314	1.36705	293.15	293.15	0	352.762	352.762	0.0801443	0.080164

298	79.74	-12.0483	20.0008	-0.0161523	1.37251	293.15	293.15	0	352.943	352.943	0.0801827	0.0802025

299	79.9	-12.084	19.9977	-0.0161992	1.37774	293.15	293.15	0	353.092	353.092	0.0802213	0.0802409

300	80.07	-12.0819	19.9935	-0.0161957	1.38391	293.15	293.15	0	353.271	353.271	0.0802602	0.0802797

301	80.24	-12.065	20.0008	-0.0161721	1.38888	293.15	293.15	0	353.44	353.44	0.0802991	0.0803184

302	80.41	-12.0744	19.9987	-0.016184	1.39112	293.15	293.15	0	353.604	353.604	0.0803378	0.0803576

303	80.57	-12.0414	19.9925	-0.0161389	1.39873	293.15	293.15	0	353.763	353.763	0.0803764	0.0803965

304	80.74	-12.0786	20.0008	-0.0161879	1.40132	293.15	293.15	0	353.932	353.932	0.0804155	0.0804355

305	80.91	-12.0816	20.0008	-0.0161912	1.40448	293.15	293.15	0	354.106	354.106	0.0804544	0.0804747

306	81.08	-12.0733	20.0008	-0.0161792	1.40917	293.15	293.15	0	354.264	354.264	0.0804921	0.0805129

307	81.24	-12.0146	20.0008	-0.0160997	1.41453	293.15	293.15	0	354.426	354.426	0.0805311	0.0805518

308	81.41	-12.0428	20.0008	-0.0161367	1.4215	293.15	293.15	0	354.602	354.602	0.0805697	0.0805909

309	81.58	-12.0068	20.0008	-0.0160877	1.42415	293.15	293.15	0	354.773	354.773	0.0806091	0.0806298

310	81.75	-11.9874	20.0071	-0.0160609	1.42756	293.15	293.15	0	354.939	354.939	0.0806483	0.0806691

311	81.91	-11.9702	20.006	-0.016037	1.43691	293.15	293.15	0	355.094	355.094	0.0806859	0.0807074

312	82.08	-11.8317	20.0008	-0.0158507	1.43698	293.15	293.15	0	355.267	355.267	0.0807255	0.0807469

313	82.25	-11.7397	20.0008	-0.0157267	1.44357	293.15	293.15	0	355.44	355.44	0.0807628	0.0807845

314	82.42	-11.7584	20.0008	-0.0157509	1.44523	293.15	293.15	0	355.595	355.595	0.0808027	0.0808239

315	82.58	-11.8149	20.0008	-0.0158258	1.45173	293.15	293.15	0	355.768	355.768	0.0808405	0.0808624

316	82.75	-11.8287	19.9956	-0.0158435	1.45765	293.15	293.15	0	355.934	355.934	0.080879	0.0809001

317	82.91	-11.8353	20.0008	-0.0158515	1.46034	293.15	293.15	0	356.091	356.091	0.0809176	0.0809391

318	83.08	-11.8643	19.9977	-0.0158895	1.46478	293.15	293.15	0	356.261	356.261	0.0809565	0.0809783

319	83.25	-11.8845	19.9904	-0.0159159	1.47244	293.15	293.15	0	356.437	356.437	0.080995	0.081017

320	83.42	-11.8602	19.9904	-0.0158825	1.4773	293.15	293.15	0	356.598	356.598	0.0810341	0.081056

321	83.58	-11.8421	19.9904	-0.0158575	1.48316	293.15	293.15	0	356.767	356.767	0.0810716	0.0810945

322	83.75	-11.8017	19.9925	-0.0158025	1.48553	293.15	293.15	0	356.935	356.935	0.0811105	0.0811337

323	83.92	-11.8055	20.0008	-0.0158069	1.48864	293.15	293.15	0	357.104	357.104	0.0811495	0.081173

324	84.09	-11.7811	20.0008	-0.0157733	1.49579	293.15	293.15	0	357.277	357.277	0.081188	0.0812118

325	84.26	-11.7495	20.0008	-0.0157302	1.49919	293.15	293.15	0	357.425	357.425	0.0812269	0.0812503

326	84.42	-11.745	20.0008	-0.0157235	1.50399	293.15	293.15	0	357.591	357.591	0.0812649	0.0812889

327	84.59	-11.7302	19.9946	-0.0157028	1.5088	293.15	293.15	0	357.772	357.772	0.0813041	0.0813282

328	84.76	-11.6864	19.9904	-0.0156435	1.51501	293.15	293.15	0	357.928	357.928	0.081343	0.0813665

329	84.92	-11.6547	20.0008	-0.0156001	1.51758	293.15	293.15	0	358.092	358.092	0.0813818	0.0814053

330	85.09	-11.6423	20.006	-0.0155828	1.52448	293.15	293.15	0	358.265	358.265	0.0814198	0.0814441

331	85.26	-11.6607	20.0071	-0.0156066	1.52859	293.15	293.15	0	358.422	358.422	0.0814577	0.0814821

332	85.43	-11.6948	20.0008	-0.0156515	1.52982	293.15	293.15	0	358.593	358.593	0.0814974	0.0815215

333	85.59	-11.7397	19.9956	-0.0157108	1.5408	293.15	293.15	0	358.768	358.768	0.0815351	0.0815594

334	85.76	-11.7232	20.0008	-0.0156879	1.54261	293.15	293.15	0	358.931	358.931	0.0815736	0.0815981

335	85.92	-11.6663	19.9977	-0.015611	1.54925	293.15	293.15	0	359.099	359.099	0.0816122	0.0816369

336	86.09	-11.6342	19.9935	-0.0155673	1.5548	293.15	293.15	0	359.27	359.27	0.0816503	0.0816755

337	86.26	-11.6317	20.0008	-0.0155632	1.55734	293.15	293.15	0	359.429	359.429	0.0816896	0.0817146

338	86.43	-11.6773	20.0008	-0.0156234	1.56481	293.15	293.15	0	359.597	359.597	0.081728	0.0817533

339	86.6	-11.6567	19.9987	-0.015595	1.56729	293.15	293.15	0	359.766	359.766	0.0817673	0.0817928

340	86.76	-11.6321	19.9914	-0.0155614	1.57175	293.15	293.15	0	359.933	359.933	0.0818053	0.0818308

341	86.93	-11.5716	20.0008	-0.0154796	1.57814	293.15	293.15	0	360.096	360.096	0.0818435	0.0818694

342	87.1	-11.5548	20.0008	-0.0154563	1.5815	293.15	293.15	0	360.269	360.269	0.0818819	0.0819082

343	87.26	-11.615	20.0008	-0.0155361	1.58792	293.15	293.15	0	360.435	360.435	0.0819211	0.0819469

344	87.43	-11.6505	20.0008	-0.0155829	1.5901	293.15	293.15	0	360.597	360.597	0.0819595	0.0819859

345	87.59	-11.6603	20.0008	-0.0155951	1.59806	293.15	293.15	0	360.765	360.765	0.0819972	0.0820235

346	87.77	-11.6457	20.0008	-0.0155748	1.60457	293.15	293.15	0	360.928	360.928	0.0820358	0.0820635

347	87.93	-11.6254	20.0008	-0.015547	1.6079	293.15	293.15	0	361.091	361.091	0.0820747	0.0821018

348	88.1	-11.6515	20.0008	-0.015581	1.61401	293.15	293.15	0	361.266	361.266	0.0821134	0.0821404

349	88.27	-11.7141	20.0008	-0.0156639	1.61496	293.15	293.15	0	361.43	361.43	0.0821528	0.0821795

350	88.44	-11.7629	20.0008	-0.0157284	1.61729	293.15	293.15	0	361.593	361.593	0.0821919	0.0822192

351	88.6	-11.7899	20.0008	-0.0157637	1.62545	293.15	293.15	0	361.766	361.766	0.0822305	0.0822573

352	88.77	-11.7476	20.0008	-0.0157064	1.63172	293.15	293.15	0	361.935	361.935	0.0822692	0.0822965

353	88.94	-11.6678	20.0008	-0.015599	1.63545	293.15	293.15	0	362.094	362.094	0.0823072	0.0823344

354	89.1	-11.5847	20.0008	-0.015487	1.63879	293.15	293.15	0	362.263	362.263	0.0823456	0.0823725

355	89.27	-11.5006	19.9935	-0.0153739	1.64594	293.15	293.15	0	362.437	362.437	0.0823839	0.0824112

356	89.44	-11.4709	19.9914	-0.0153334	1.65012	293.15	293.15	0	362.595	362.595	0.0824222	0.0824497

357	89.6	-11.4326	19.9998	-0.0152814	1.65464	293.15	293.15	0	362.766	362.766	0.0824617	0.0824885

358	89.77	-11.4038	19.9966	-0.0152421	1.66005	293.15	293.15	0	362.933	362.933	0.0824993	0.0825271

359	89.94	-11.4271	20.0008	-0.0152724	1.66575	293.15	293.15	0	363.104	363.104	0.0825382	0.0825666

360	90.11	-11.4939	20.0008	-0.015361	1.67307	293.15	293.15	0	363.27	363.27	0.082576	0.0826046

361	90.27	-11.5808	19.9956	-0.0154764	1.67664	293.15	293.15	0	363.425	363.425	0.0826143	0.0826433

362	90.44	-11.5908	19.9904	-0.0154889	1.67892	293.15	293.15	0	363.607	363.607	0.0826542	0.0826823

363	90.61	-11.5177	20.0008	-0.0153905	1.68294	293.15	293.15	0	363.771	363.771	0.082692	0.0827203

364	90.77	-11.3678	20.0008	-0.0151895	1.6864	293.15	293.15	0	363.937	363.937	0.0827307	0.0827589

365	90.94	-11.2923	20.0008	-0.0150878	1.6971	293.15	293.15	0	364.099	364.099	0.0827688	0.0827977

366	91.1	-11.2953	20.0102	-0.0150911	1.69964	293.15	293.15	0	364.265	364.265	0.0828065	0.0828353

367	91.27	-11.2882	20.0071	-0.0150809	1.7031	293.15	293.15	0	364.438	364.438	0.0828458	0.0828737

368	91.44	-11.2826	20.0008	-0.0150726	1.70852	293.15	293.15	0	364.6	364.6	0.0828842	0.0829126

369	91.61	-11.3696	20.0008	-0.015188	1.71626	293.15	293.15	0	364.768	364.768	0.0829227	0.0829524

370	91.78	-11.4462	20.0008	-0.0152896	1.72136	293.15	293.15	0	364.929	364.929	0.0829614	0.0829913

371	91.94	-11.4865	20.0008	-0.0153427	1.72682	293.15	293.15	0	365.098	365.098	0.0829987	0.0830289

372	92.11	-11.4724	20.0008	-0.0153231	1.73017	293.15	293.15	0	365.266	365.266	0.0830377	0.083068

373	92.28	-11.4188	20.0008	-0.0152507	1.73791	293.15	293.15	0	365.435	365.435	0.0830762	0.0831064

374	92.44	-11.3141	20.0008	-0.0151101	1.74293	293.15	293.15	0	365.603	365.603	0.0831141	0.0831447

375	92.61	-11.2431	19.9998	-0.0150146	1.74412	293.15	293.15	0	365.765	365.765	0.0831545	0.083184

376	92.78	-11.2249	19.9914	-0.0149894	1.75059	293.15	293.15	0	365.929	365.929	0.0831922	0.0832222

377	92.95	-11.2369	20.0008	-0.0150048	1.75757	293.15	293.15	0	366.104	366.104	0.0832306	0.0832612

378	93.11	-11.2951	20.0008	-0.0150817	1.76562	293.15	293.15	0	366.266	366.266	0.0832676	0.0832987

379	93.28	-11.3401	20.0008	-0.0151411	1.7688	293.15	293.15	0	366.432	366.432	0.0833064	0.0833378

380	93.45	-11.3502	20.0008	-0.0151538	1.77065	293.15	293.15	0	366.597	366.597	0.0833462	0.0833777

381	93.61	-11.2985	20.0008	-0.015084	1.77685	293.15	293.15	0	366.769	366.769	0.0833844	0.0834154

382	93.78	-11.2156	20.0008	-0.0149726	1.7823	293.15	293.15	0	366.934	366.934	0.0834231	0.0834544

383	93.95	-11.1698	20.0008	-0.0149107	1.78563	293.15	293.15	0	367.099	367.099	0.0834618	0.0834933

384	94.12	-11.093	20.0008	-0.0148074	1.78957	293.15	293.15	0	367.261	367.261	0.0834998	0.0835315

385	94.28	-11.0259	20.0008	-0.0147171	1.79592	293.15	293.15	0	367.43	367.43	0.0835384	0.0835702

386	94.45	-11.0496	20.0008	-0.0147479	1.80283	293.15	293.15	0	367.599	367.599	0.0835765	0.0836089

387	94.62	-11.1318	20.0008	-0.014857	1.80872	293.15	293.15	0	367.767	367.767	0.0836152	0.0836477

388	94.79	-11.2102	20.0008	-0.0149609	1.81465	293.15	293.15	0	367.936	367.936	0.083653	0.0836858

389	94.95	-11.2638	19.9987	-0.0150317	1.81792	293.15	293.15	0	368.096	368.096	0.0836916	0.0837244

390	95.12	-11.3051	19.9925	-0.015086	1.82248	293.15	293.15	0	368.261	368.261	0.0837312	0.083764

391	95.29	-11.2832	20.0008	-0.015056	1.82737	293.15	293.15	0	368.433	368.433	0.0837699	0.0838022

392	95.46	-11.2617	20.0008	-0.0150265	1.83193	293.15	293.15	0	368.601	368.601	0.0838081	0.0838409

393	95.62	-11.1385	20.0008	-0.0148614	1.83729	293.15	293.15	0	368.763	368.763	0.0838464	0.0838793

394	95.79	-11.0314	20.0071	-0.0147178	1.84413	293.15	293.15	0	368.93	368.93	0.0838844	0.0839178

395	95.96	-11.0352	20.0102	-0.0147222	1.84868	293.15	293.15	0	369.101	369.101	0.0839227	0.0839563

396	96.12	-11.0518	20.0008	-0.0147436	1.8543	293.15	293.15	0	369.267	369.267	0.0839609	0.0839935

397	96.29	-11.0431	19.9956	-0.0147313	1.86178	293.15	293.15	0	369.423	369.423	0.0839983	0.0840323

398	96.45	-11.0259	20.0008	-0.0147075	1.86583	293.15	293.15	0	369.595	369.595	0.0840367	0.0840704

399	96.62	-11.0598	20.0008	-0.014752	1.86939	293.15	293.15	0	369.768	369.768	0.0840763	0.0841103

400	96.79	-11.0625	20.0008	-0.0147549	1.8752	293.15	293.15	0	369.932	369.932	0.084115	0.0841487

401	96.96	-11.0336	20.0008	-0.0147156	1.87958	293.15	293.15	0	370.089	370.089	0.0841528	0.0841874

402	97.13	-11.0214	20.0008	-0.0146986	1.88172	293.15	293.15	0	370.26	370.26	0.0841924	0.0842266

403	97.3	-11.0012	20.0008	-0.0146709	1.88961	293.15	293.15	0	370.435	370.435	0.0842313	0.084265

404	97.46	-10.9502	20.0008	-0.0146021	1.89293	293.15	293.15	0	370.607	370.607	0.0842692	0.0843029

405	97.62	-10.8186	19.9977	-0.014426	1.90092	293.15	293.15	0	370.765	370.765	0.0843068	0.0843407

406	97.79	-10.7234	19.9935	-0.0142984	1.90725	293.15	293.15	0	370.936	370.936	0.0843449	0.0843793

407	97.96	-10.7283	20.0008	-0.0143041	1.91365	293.15	293.15	0	371.102	371.102	0.0843829	0.0844178

408	98.12	-10.806	20.0008	-0.0144069	1.92014	293.15	293.15	0	371.269	371.269	0.0844212	0.0844562

409	98.29	-10.8757	20.0008	-0.0144992	1.92233	293.15	293.15	0	371.424	371.424	0.0844607	0.0844945

410	98.46	-10.8585	20.0008	-0.0144755	1.92655	293.15	293.15	0	371.591	371.591	0.0844987	0.0845335

411	98.63	-10.8075	20.0008	-0.0144068	1.9334	293.15	293.15	0	371.761	371.761	0.0845365	0.0845717

412	98.79	-10.7868	20.0008	-0.0143785	1.9401	293.15	293.15	0	371.928	371.928	0.0845742	0.08461

413	98.96	-10.7598	20.0008	-0.0143418	1.94464	293.15	293.15	0	372.1	372.1	0.0846133	0.0846479

414	99.13	-10.7293	20.0071	-0.0143004	1.9472	293.15	293.15	0	372.266	372.266	0.0846527	0.0846876

415	99.3	-10.7259	20.0112	-0.0142951	1.95404	293.15	293.15	0	372.421	372.421	0.0846909	0.0847265

416	99.46	-10.7385	20.0008	-0.0143112	1.96412	293.15	293.15	0	372.602	372.602	0.0847276	0.0847645

417	99.63	-10.693	20.0008	-0.0142499	1.96307	293.15	293.15	0	372.767	372.767	0.0847674	0.0848035

418	99.8	-10.6397	20.0008	-0.0141782	1.96983	293.15	293.15	0	372.93	372.93	0.0848056	0.0848421

419	99.97	-10.6127	19.9966	-0.0141416	1.97373	293.15	293.15	0	373.096	373.096	0.0848438	0.0848802

420	100.13	-10.6525	19.9946	-0.0141938	1.8934	293.15	293.15	0	373.064	373.064	0.0848824	0.0849184

421	100.26	-10.7631	20.0008	-0.0143406	1.76519	293.15	293.15	0	372.893	372.893	0.0849128	0.084949

422	100.32	-10.6253	20.0008	-0.0141568	1.65841	293.15	293.15	0	372.73	372.73	0.0849277	0.084961

423	100.29	-9.57533	20.0008	-0.012758	1.57367	293.15	293.15	0	372.571	372.571	0.0849252	0.0849554

424	100.21	-7.63288	19.9925	-0.0101701	1.49592	293.15	293.15	0	372.393	372.393	0.0849098	0.0849356

425	100.07	-5.12799	19.9925	-0.00683287	1.44156	293.15	293.15	0	372.242	372.242	0.0848843	0.084905

426	99.91	-2.42738	20.0008	-0.00323456	1.3928	293.15	293.15	0	372.078	372.078	0.0848511	0.0848683

427	99.72	0.290698	20.0008	0.000387385	1.35605	293.15	293.15	0	371.904	371.904	0.0848112	0.0848244

428	99.52	2.89895	19.9987	0.00386338	1.32831	293.15	293.15	0	371.737	371.737	0.0847669	0.0847773

429	99.3	5.29558	19.9914	0.00705781	1.30419	293.15	293.15	0	371.584	371.584	0.0847199	0.0847272

430	99.08	7.40243	20.0008	0.00986642	1.29058	293.15	293.15	0	371.409	371.409	0.0846696	0.0846752

431	98.85	9.13715	20.0008	0.0121794	1.27831	293.15	293.15	0	371.238	371.238	0.0846191	0.0846229

432	98.61	10.6307	20.0008	0.0141712	1.27186	293.15	293.15	0	371.071	371.071	0.0845662	0.084568

433	98.38	11.7837	20.0008	0.0157092	1.26675	293.15	293.15	0	370.917	370.917	0.0845141	0.0845156

434	98.15	12.6794	20.0008	0.0169046	1.26857	293.15	293.15	0	370.735	370.735	0.0844602	0.0844609

435	97.92	13.3494	20.0008	0.0177991	1.26602	293.15	293.15	0	370.571	370.571	0.0844095	0.0844088

436	97.7	13.7576	20.0008	0.0183445	1.26976	293.15	293.15	0	370.406	370.406	0.0843589	0.084359

437	97.49	14.0026	20.0008	0.0186723	1.27159	293.15	293.15	0	370.242	370.242	0.084309	0.0843092

438	97.28	14.1475	19.9966	0.0188668	1.2701	293.15	293.15	0	370.076	370.076	0.0842615	0.0842615

439	97.07	14.1574	19.9946	0.0188811	1.27378	293.15	293.15	0	369.903	369.903	0.0842131	0.0842126

440	96.87	14.0317	20.0008	0.0187147	1.27691	293.15	293.15	0	369.74	369.74	0.0841664	0.0841664

441	96.68	13.7846	20.0008	0.0183862	1.2734	293.15	293.15	0	369.566	369.566	0.0841221	0.0841222

442	96.48	13.5522	19.9977	0.0180772	1.27314	293.15	293.15	0	369.4	369.4	0.084077	0.0840774

443	96.3	13.3894	19.9925	0.017861	1.27062	293.15	293.15	0	369.243	369.243	0.0840349	0.0840355

444	96.12	13.1767	20.0008	0.0175783	1.27004	293.15	293.15	0	369.075	369.075	0.0839924	0.0839927

445	95.93	12.9969	20.0008	0.0173394	1.27235	293.15	293.15	0	368.906	368.906	0.0839498	0.0839493

446	95.75	12.8066	20.0008	0.0170864	1.27117	293.15	293.15	0	368.729	368.729	0.0839087	0.0839088

447	95.57	12.584	20.0008	0.0167904	1.26915	293.15	293.15	0	368.576	368.576	0.083868	0.083868

448	95.4	12.3375	20.0019	0.0164623	1.26582	293.15	293.15	0	368.401	368.401	0.0838268	0.083828

449	95.23	12.1066	20.005	0.016155	1.26432	293.15	293.15	0	368.23	368.23	0.083787	0.0837879

450	95.05	11.958	20.0008	0.0159575	1.2625	293.15	293.15	0	368.063	368.063	0.083747	0.0837476

451	94.89	11.7977	20.0008	0.0157445	1.25575	293.15	293.15	0	367.909	367.909	0.0837084	0.083709

452	94.72	11.6145	20.0008	0.0155008	1.25262	293.15	293.15	0	367.726	367.726	0.083669	0.0836699

453	94.55	11.456	20.0008	0.01529	1.25077	293.15	293.15	0	367.579	367.579	0.0836298	0.0836312

454	94.38	11.3019	20.0008	0.0150851	1.24626	293.15	293.15	0	367.405	367.405	0.0835916	0.0835932

455	94.21	11.1401	19.9966	0.0148698	1.24513	293.15	293.15	0	367.235	367.235	0.0835523	0.0835541

456	94.05	11.0038	19.9935	0.0146887	1.23571	293.15	293.15	0	367.066	367.066	0.0835147	0.0835158

457	93.88	10.9104	20.0008	0.0145647	1.23424	293.15	293.15	0	366.912	366.912	0.0834758	0.0834772

458	93.72	10.8328	20.0008	0.0144619	1.22715	293.15	293.15	0	366.741	366.741	0.0834376	0.0834391

459	93.55	10.7696	20.0008	0.0143782	1.22035	293.15	293.15	0	366.565	366.565	0.0833999	0.0834009

460	93.38	10.7635	20.0008	0.0143708	1.21613	293.15	293.15	0	366.405	366.405	0.083361	0.0833614

461	93.21	10.8276	19.9987	0.0144571	1.21097	293.15	293.15	0	366.244	366.244	0.0833231	0.0833229

462	93.05	10.8682	19.9904	0.0145121	1.20877	293.15	293.15	0	366.071	366.071	0.0832843	0.0832843

463	92.88	10.9205	19.9977	0.0145826	1.20609	293.15	293.15	0	365.904	365.904	0.0832456	0.0832452

464	92.71	10.9551	20.0008	0.0146295	1.19774	293.15	293.15	0	365.734	365.734	0.0832072	0.0832071

465	92.54	10.969	20.0008	0.0146488	1.19546	293.15	293.15	0	365.577	365.577	0.0831685	0.0831681

466	92.37	10.9417	20.0008	0.0146131	1.19298	293.15	293.15	0	365.412	365.412	0.0831294	0.0831291

467	92.21	10.907	20.0008	0.0145674	1.18811	293.15	293.15	0	365.228	365.228	0.0830913	0.0830908

468	92.05	10.9065	20.0008	0.0145675	1.18161	293.15	293.15	0	365.065	365.065	0.0830539	0.0830534

469	91.88	10.9065	19.9956	0.0145682	1.17431	293.15	293.15	0	364.901	364.901	0.0830154	0.0830143

470	91.71	10.881	20.0008	0.0145349	1.17007	293.15	293.15	0	364.728	364.728	0.082977	0.082976

471	91.54	10.881	20.0008	0.0145356	1.16652	293.15	293.15	0	364.571	364.571	0.0829383	0.0829366

472	91.37	10.9546	20.0008	0.0146347	1.16369	293.15	293.15	0	364.398	364.398	0.0828997	0.0828976

473	91.21	10.9798	20.0008	0.0146691	1.15745	293.15	293.15	0	364.245	364.245	0.0828606	0.08286

474	91.04	10.8968	20.0008	0.0145589	1.15143	293.15	293.15	0	364.062	364.062	0.0828219	0.082821

475	90.88	10.7856	20.0008	0.0144111	1.14738	293.15	293.15	0	363.911	363.911	0.0827833	0.0827827

476	90.71	10.7057	20.0008	0.014305	1.14226	293.15	293.15	0	363.735	363.735	0.0827464	0.0827446

477	90.54	10.6505	20.0008	0.0142319	1.13895	293.15	293.15	0	363.565	363.565	0.0827075	0.0827062

478	90.38	10.639	19.9987	0.0142173	1.13117	293.15	293.15	0	363.4	363.4	0.0826692	0.0826676

479	90.21	10.6528	19.9914	0.0142365	1.1281	293.15	293.15	0	363.242	363.242	0.0826301	0.0826288

480	90.04	10.6218	19.9946	0.0141958	1.12363	293.15	293.15	0	363.071	363.071	0.0825914	0.0825898

481	89.88	10.6104	19.9914	0.0141812	1.11641	293.15	293.15	0	362.898	362.898	0.0825538	0.0825518

482	89.7	10.6382	20.0008	0.0142192	1.11123	293.15	293.15	0	362.741	362.741	0.0825151	0.0825119

483	89.54	10.6339	19.9956	0.0142141	1.10646	293.15	293.15	0	362.577	362.577	0.0824765	0.0824737

484	89.37	10.5856	19.9904	0.0141502	1.10552	293.15	293.15	0	362.404	362.404	0.0824369	0.0824345

485	89.21	10.5703	19.9904	0.0141304	1.09916	293.15	293.15	0	362.23	362.23	0.0823991	0.0823968

486	89.04	10.6266	20.0008	0.0142065	1.09663	293.15	293.15	0	362.066	362.066	0.08236	0.0823576

487	88.87	10.7263	20.0008	0.0143405	1.08898	293.15	293.15	0	361.909	361.909	0.082322	0.0823184

488	88.7	10.7306	20.0008	0.0143469	1.08611	293.15	293.15	0	361.729	361.729	0.0822833	0.0822796

489	88.53	10.7094	20.0008	0.0143194	1.08243	293.15	293.15	0	361.563	361.563	0.0822442	0.0822404

490	88.37	10.6727	20.0008	0.014271	1.07683	293.15	293.15	0	361.391	361.391	0.0822058	0.0822027

491	88.2	10.6331	20.0008	0.0142187	1.07076	293.15	293.15	0	361.233	361.233	0.0821672	0.0821636

492	88.03	10.6371	20.0008	0.0142248	1.06643	293.15	293.15	0	361.069	361.069	0.0821285	0.0821244

493	87.86	10.6402	20.0008	0.0142297	1.0607	293.15	293.15	0	360.912	360.912	0.0820902	0.0820862

494	87.7	10.6647	20.0008	0.0142631	1.05721	293.15	293.15	0	360.744	360.744	0.0820515	0.0820474

495	87.53	10.7019	20.0008	0.0143137	1.05429	293.15	293.15	0	360.566	360.566	0.082013	0.0820089

496	87.36	10.7255	19.9998	0.0143459	1.04823	293.15	293.15	0	360.408	360.408	0.0819742	0.08197

497	87.19	10.7144	19.9966	0.0143318	1.04462	293.15	293.15	0	360.245	360.245	0.0819353	0.0819308

498	87.03	10.6788	20.0008	0.0142848	1.03906	293.15	293.15	0	360.071	360.071	0.0818974	0.0818926

499	86.86	10.6008	20.0008	0.0141812	1.03785	293.15	293.15	0	359.906	359.906	0.0818581	0.0818531

500	86.69	10.6012	20.0008	0.0141826	1.032	293.15	293.15	0	359.743	359.743	0.0818191	0.0818143

501	86.52	10.6549	20.0008	0.014255	1.02462	293.15	293.15	0	359.569	359.569	0.0817808	0.0817755

502	86.36	10.7197	20.0008	0.0143424	1.02196	293.15	293.15	0	359.405	359.405	0.0817423	0.0817372

503	86.19	10.8304	20.0008	0.0144913	1.01477	293.15	293.15	0	359.239	359.239	0.0817046	0.081698

504	86.02	10.9272	20.0008	0.0146215	1.01424	293.15	293.15	0	359.066	359.066	0.0816653	0.0816584

505	85.85	10.9158	20.0008	0.0146071	1.0087	293.15	293.15	0	358.908	358.908	0.0816259	0.0816195

506	85.68	10.8554	20.0008	0.0145269	1.00411	293.15	293.15	0	358.739	358.739	0.0815874	0.0815807

507	85.51	10.7774	20.0008	0.0144233	0.998939	293.15	293.15	0	358.563	358.563	0.0815483	0.0815419

508	85.35	10.6774	20.0008	0.0142903	0.994147	293.15	293.15	0	358.402	358.402	0.0815104	0.0815036

509	85.18	10.5905	20.0008	0.0141747	0.98888	293.15	293.15	0	358.242	358.242	0.0814727	0.0814653

510	85.02	10.5644	20.0008	0.0141404	0.983709	293.15	293.15	0	358.065	358.065	0.0814335	0.0814263

511	84.85	10.5882	20.0008	0.014173	0.979403	293.15	293.15	0	357.896	357.896	0.0813954	0.0813874

512	84.68	10.6716	20.0019	0.0142853	0.973891	293.15	293.15	0	357.73	357.73	0.0813569	0.0813487

513	84.51	10.8438	20.0102	0.0145166	0.971482	293.15	293.15	0	357.574	357.574	0.081318	0.0813092

514	84.34	10.9529	20.0008	0.0146633	0.967572	293.15	293.15	0	357.409	357.409	0.0812779	0.0812704

515	84.17	10.9515	20.0008	0.0146623	0.961552	293.15	293.15	0	357.245	357.245	0.0812394	0.0812312

516	84.01	10.9151	20.0008	0.0146142	0.958952	293.15	293.15	0	357.072	357.072	0.0812006	0.0811926

517	83.84	10.8401	19.9956	0.0145146	0.956222	293.15	293.15	0	356.898	356.898	0.0811618	0.0811533

518	83.68	10.8715	19.9904	0.0145574	0.952206	293.15	293.15	0	356.733	356.733	0.0811242	0.0811157

519	83.5	10.8928	19.9998	0.0145866	0.94483	293.15	293.15	0	356.571	356.571	0.0810849	0.0810762

520	83.34	10.9309	20.0008	0.0146384	0.941853	293.15	293.15	0	356.404	356.404	0.0810466	0.0810375

521	83.17	10.946	20.0008	0.0146593	0.938159	293.15	293.15	0	356.231	356.231	0.0810086	0.0809996

522	83	10.9151	20.0008	0.0146187	0.933663	293.15	293.15	0	356.068	356.068	0.0809686	0.0809592

523	82.83	10.8556	20.0008	0.0145397	0.926852	293.15	293.15	0	355.901	355.901	0.0809303	0.0809209

524	82.67	10.7608	20.0008	0.0144134	0.922177	293.15	293.15	0	355.732	355.732	0.0808921	0.0808826

525	82.5	10.7049	20.0008	0.0143392	0.917498	293.15	293.15	0	355.563	355.563	0.0808528	0.0808429

526	82.34	10.7277	20.0008	0.0143706	0.914249	293.15	293.15	0	355.399	355.399	0.0808158	0.0808054

527	82.16	10.7348	20.0008	0.0143809	0.908327	293.15	293.15	0	355.239	355.239	0.0807754	0.0807653

528	82	10.8127	20.0008	0.0144858	0.905975	293.15	293.15	0	355.07	355.07	0.0807368	0.0807262

529	81.83	10.8404	20.0008	0.0145238	0.903104	293.15	293.15	0	354.897	354.897	0.0806983	0.0806873

530	81.66	10.7653	20.0008	0.0144238	0.900987	293.15	293.15	0	354.738	354.738	0.0806584	0.0806486

531	81.49	10.7438	20.0019	0.0143958	0.894137	293.15	293.15	0	354.576	354.576	0.0806206	0.0806099

532	81.33	10.7775	20.0102	0.0144416	0.886491	293.15	293.15	0	354.401	354.401	0.0805824	0.0805708

533	81.16	10.8038	20.0008	0.0144776	0.883718	293.15	293.15	0	354.23	354.23	0.0805439	0.0805324

534	80.99	10.8603	20.0008	0.014554	0.880675	293.15	293.15	0	354.064	354.064	0.0805042	0.080494

535	80.82	10.9117	20.0008	0.0146237	0.875013	293.15	293.15	0	353.899	353.899	0.0804656	0.0804544

536	80.66	10.8998	20.0008	0.0146084	0.870169	293.15	293.15	0	353.735	353.735	0.0804276	0.0804169

537	80.5	10.8384	20.0008	0.0145269	0.868068	293.15	293.15	0	353.569	353.569	0.0803884	0.0803783

538	80.33	10.7493	20.0008	0.0144082	0.861397	293.15	293.15	0	353.399	353.399	0.0803505	0.0803395

539	80.16	10.7138	19.9977	0.0143614	0.857253	293.15	293.15	0	353.249	353.249	0.0803112	0.0803006

540	79.99	10.7712	19.9935	0.014439	0.852696	293.15	293.15	0	353.07	353.07	0.0802726	0.080261

541	79.83	10.7952	20.0008	0.0144719	0.848933	293.15	293.15	0	352.902	352.902	0.0802335	0.0802225

542	79.66	10.7846	20.0008	0.0144585	0.844498	293.15	293.15	0	352.729	352.729	0.0801947	0.0801831

543	79.49	10.8376	20.0008	0.0145302	0.840801	293.15	293.15	0	352.578	352.578	0.0801565	0.0801449

544	79.32	10.855	20.0008	0.0145543	0.837637	293.15	293.15	0	352.409	352.409	0.0801172	0.080105

545	79.15	10.8559	19.9987	0.0145562	0.831875	293.15	293.15	0	352.236	352.236	0.0800785	0.0800659

546	78.99	10.8732	19.9914	0.0145801	0.828542	293.15	293.15	0	352.077	352.077	0.0800401	0.0800276

547	78.81	10.8932	20.0008	0.0146077	0.826303	293.15	293.15	0	351.905	351.905	0.0800009	0.0799878

548	78.65	10.8895	20.0008	0.0146034	0.820476	293.15	293.15	0	351.739	351.739	0.079963	0.0799501

549	78.48	10.8574	20.0008	0.0145612	0.815708	293.15	293.15	0	351.568	351.568	0.0799236	0.0799105

550	78.31	10.8956	20.0008	0.0146131	0.812207	293.15	293.15	0	351.403	351.403	0.0798841	0.0798708

551	78.15	10.9279	20.0008	0.0146572	0.808436	293.15	293.15	0	351.238	351.238	0.0798468	0.0798325

552	77.98	10.8898	20.0008	0.0146068	0.804186	293.15	293.15	0	351.065	351.065	0.0798077	0.0797932

553	77.81	10.8599	20.0008	0.0145674	0.798394	293.15	293.15	0	350.901	350.901	0.0797691	0.0797549

554	77.64	10.8211	20.0008	0.0145162	0.794118	293.15	293.15	0	350.728	350.728	0.07973	0.0797155

555	77.47	10.8391	20.0008	0.014541	0.791452	293.15	293.15	0	350.571	350.571	0.079691	0.0796764

556	77.31	10.873	20.0008	0.0145873	0.787197	293.15	293.15	0	350.398	350.398	0.0796531	0.0796388

557	77.15	10.8797	20.0008	0.014597	0.782181	293.15	293.15	0	350.244	350.244	0.0796143	0.0795999

558	76.98	10.8728	20.0008	0.0145885	0.777231	293.15	293.15	0	350.068	350.068	0.0795751	0.0795611

559	76.81	10.8662	20.0008	0.0145803	0.772417	293.15	293.15	0	349.898	349.898	0.0795363	0.0795222

560	76.64	10.8376	20.0008	0.0145426	0.767441	293.15	293.15	0	349.739	349.739	0.0794975	0.0794832

561	76.48	10.8315	20.0008	0.0145351	0.763946	293.15	293.15	0	349.574	349.574	0.0794599	0.0794448

562	76.31	10.7507	20.0008	0.0144275	0.757505	293.15	293.15	0	349.406	349.406	0.0794208	0.0794057

563	76.14	10.6828	20.0008	0.0143371	0.755168	293.15	293.15	0	349.228	349.228	0.0793819	0.079367

564	75.97	10.6774	20.0008	0.0143306	0.751353	293.15	293.15	0	349.068	349.068	0.0793428	0.0793273

565	75.8	10.7159	20.0008	0.014383	0.749132	293.15	293.15	0	348.906	348.906	0.0793032	0.079287

566	75.64	10.7582	19.9946	0.0144405	0.743181	293.15	293.15	0	348.731	348.731	0.0792654	0.0792488

567	75.46	10.7785	19.9966	0.0144685	0.740584	293.15	293.15	0	348.561	348.561	0.0792248	0.0792089

568	75.3	10.8225	20.0008	0.0145283	0.735299	293.15	293.15	0	348.405	348.405	0.0791867	0.0791713

569	75.13	10.8579	20.006	0.0145766	0.731959	293.15	293.15	0	348.24	348.24	0.0791486	0.0791321

570	74.97	10.8862	19.9956	0.0146153	0.726733	293.15	293.15	0	348.067	348.067	0.0791092	0.079093

571	74.8	10.8734	19.9904	0.0145988	0.722677	293.15	293.15	0	347.902	347.902	0.0790703	0.0790546

572	74.63	10.8298	20.0008	0.014541	0.72152	293.15	293.15	0	347.739	347.739	0.079031	0.0790155

573	74.47	10.7805	20.0008	0.0144756	0.715721	293.15	293.15	0	347.572	347.572	0.0789933	0.0789768

574	74.3	10.6971	20.0008	0.0143643	0.715063	293.15	293.15	0	347.4	347.4	0.0789537	0.0789377

575	74.13	10.6379	20.0008	0.0142855	0.710588	293.15	293.15	0	347.242	347.242	0.0789146	0.0788986

576	73.97	10.6258	20.0008	0.0142699	0.703852	293.15	293.15	0	347.073	347.073	0.0788769	0.0788602

577	73.8	10.6864	20.0008	0.0143521	0.698494	293.15	293.15	0	346.904	346.904	0.078838	0.0788212

578	73.63	10.7677	19.9987	0.014462	0.693242	293.15	293.15	0	346.736	346.736	0.0788	0.0787832

579	73.46	10.7366	19.9925	0.0144209	0.690719	293.15	293.15	0	346.575	346.575	0.0787602	0.0787434

580	73.3	10.6747	20.0008	0.0143386	0.687459	293.15	293.15	0	346.408	346.408	0.0787212	0.0787044

581	73.13	10.6267	20.0008	0.0142748	0.682674	293.15	293.15	0	346.245	346.245	0.0786826	0.0786657

582	72.96	10.6046	20.0008	0.0142459	0.679466	293.15	293.15	0	346.07	346.07	0.0786438	0.078626

583	72.79	10.6312	20.0008	0.0142823	0.67309	293.15	293.15	0	345.898	345.898	0.0786051	0.0785872

584	72.62	10.6984	20.0008	0.0143733	0.669562	293.15	293.15	0	345.733	345.733	0.0785659	0.0785481

585	72.46	10.7367	20.0008	0.0144254	0.665219	293.15	293.15	0	345.577	345.577	0.078527	0.0785092

586	72.29	10.7428	19.9956	0.0144344	0.663424	293.15	293.15	0	345.405	345.405	0.0784881	0.0784709

587	72.12	10.6956	19.9956	0.0143717	0.660044	293.15	293.15	0	345.232	345.232	0.0784488	0.0784311

588	71.96	10.6322	20.0008	0.0142872	0.656197	293.15	293.15	0	345.066	345.066	0.0784111	0.0783931

589	71.79	10.6413	20.0008	0.0143001	0.650057	293.15	293.15	0	344.902	344.902	0.0783717	0.0783531

590	71.62	10.6689	20.0008	0.0143379	0.646504	293.15	293.15	0	344.74	344.74	0.0783331	0.0783146

591	71.46	10.6699	20.0008	0.01434	0.640738	293.15	293.15	0	344.563	344.563	0.0782942	0.0782757

592	71.29	10.6185	20.0008	0.0142717	0.637474	293.15	293.15	0	344.402	344.402	0.0782561	0.0782372

593	71.12	10.6205	20.0008	0.0142751	0.63322	293.15	293.15	0	344.242	344.242	0.0782171	0.0781979

594	70.95	10.7274	20.0008	0.0144196	0.628445	293.15	293.15	0	344.064	344.064	0.0781775	0.0781583

595	70.78	10.8165	20.0008	0.0145401	0.627174	293.15	293.15	0	343.912	343.912	0.0781383	0.0781181

596	70.61	10.8612	20.0008	0.0146008	0.621871	293.15	293.15	0	343.737	343.737	0.0781001	0.0780798

597	70.45	10.8706	20.0008	0.0146142	0.617405	293.15	293.15	0	343.58	343.58	0.0780595	0.0780406

598	70.28	10.855	20.0008	0.014594	0.6181	293.15	293.15	0	343.408	343.408	0.0780212	0.0780019

599	70.12	10.8139	20.0008	0.0145395	0.609382	293.15	293.15	0	343.236	343.236	0.0779834	0.0779634

600	69.95	10.8361	20.0008	0.0145701	0.605527	293.15	293.15	0	343.062	343.062	0.0779446	0.0779239

601	69.78	10.8118	20.0008	0.0145382	0.603331	293.15	293.15	0	342.906	342.906	0.0779058	0.0778853

602	69.61	10.7913	20.0008	0.0145113	0.60064	293.15	293.15	0	342.735	342.735	0.0778669	0.0778456

603	69.44	10.7727	20.0008	0.014487	0.593885	293.15	293.15	0	342.568	342.568	0.0778277	0.0778068

604	69.28	10.7723	19.9977	0.0144873	0.58974	293.15	293.15	0	342.402	342.402	0.0777895	0.0777682

605	69.11	10.7593	20.0071	0.0144705	0.586427	293.15	293.15	0	342.242	342.242	0.0777508	0.0777289

606	68.94	10.7587	20.0081	0.0144703	0.581287	293.15	293.15	0	342.065	342.065	0.0777111	0.0776901

607	68.77	10.6987	20.0008	0.0143905	0.578754	293.15	293.15	0	341.901	341.901	0.0776716	0.0776507

608	68.61	10.6591	20.0008	0.0143379	0.574771	293.15	293.15	0	341.741	341.741	0.0776332	0.0776117

609	68.44	10.6792	20.0008	0.0143657	0.571561	293.15	293.15	0	341.571	341.571	0.0775936	0.0775718

610	68.27	10.7748	19.9987	0.014495	0.568472	293.15	293.15	0	341.404	341.404	0.0775555	0.0775333

611	68.1	10.869	19.9977	0.0146224	0.56148	293.15	293.15	0	341.234	341.234	0.0775161	0.0774944

612	67.93	10.9408	20.0008	0.0147198	0.558099	293.15	293.15	0	341.067	341.067	0.0774779	0.0774546

613	67.77	10.9789	19.9998	0.0147718	0.556198	293.15	293.15	0	340.904	340.904	0.0774387	0.0774162

614	67.6	10.9898	19.9966	0.0147872	0.554231	293.15	293.15	0	340.731	340.731	0.0773987	0.0773764

615	67.43	10.9759	20.0008	0.0147693	0.544177	293.15	293.15	0	340.566	340.566	0.0773607	0.0773373

616	67.26	10.988	20.0008	0.0147863	0.539854	293.15	293.15	0	340.403	340.403	0.0773227	0.0772985

617	67.09	10.9969	20.0008	0.014799	0.54089	293.15	293.15	0	340.237	340.237	0.0772826	0.0772585

618	66.93	11.0257	20.0008	0.0148385	0.5359	293.15	293.15	0	340.064	340.064	0.0772437	0.0772195

619	66.76	10.9764	19.9956	0.014773	0.531433	293.15	293.15	0	339.9	339.9	0.0772044	0.0771802

620	66.59	10.8776	20.0008	0.0146407	0.527001	293.15	293.15	0	339.735	339.735	0.0771661	0.0771417

621	66.43	10.7944	20.0008	0.0145295	0.524689	293.15	293.15	0	339.569	339.569	0.0771274	0.0771031

622	66.26	10.7577	20.0008	0.0144808	0.522632	293.15	293.15	0	339.399	339.399	0.0770879	0.0770633

623	66.09	10.7738	20.0008	0.0145031	0.518248	293.15	293.15	0	339.239	339.239	0.0770494	0.0770244

624	65.92	10.8381	19.9977	0.0145905	0.512542	293.15	293.15	0	339.07	339.07	0.0770099	0.0769851

625	65.76	10.9301	19.9967	0.0147151	0.508694	293.15	293.15	0	338.902	338.902	0.0769714	0.0769466

626	65.59	10.9107	20.0091	0.0146898	0.503494	293.15	293.15	0	338.733	338.733	0.0769329	0.0769079

627	65.42	10.8761	19.9987	0.0146439	0.501302	293.15	293.15	0	338.573	338.573	0.0768939	0.0768682

628	65.25	10.8689	19.9977	0.0146349	0.498682	293.15	293.15	0	338.399	338.399	0.0768547	0.0768288

629	65.08	10.8822	20.0008	0.0146536	0.492665	293.15	293.15	0	338.231	338.231	0.0768149	0.0767892

630	64.92	10.9	20.0008	0.0146782	0.490826	293.15	293.15	0	338.072	338.072	0.0767763	0.0767505

631	64.75	10.9483	20.0008	0.0147441	0.486409	293.15	293.15	0	337.905	337.905	0.0767376	0.0767118

632	64.58	11.0464	20.0008	0.0148769	0.483585	293.15	293.15	0	337.74	337.74	0.0766984	0.0766721

633	64.41	11.1332	20.0008	0.0149946	0.476623	293.15	293.15	0	337.575	337.575	0.0766599	0.0766326

634	64.25	11.1385	20.0008	0.0150025	0.476523	293.15	293.15	0	337.411	337.411	0.0766207	0.0765933

635	64.08	11.1329	20.0008	0.0149957	0.472876	293.15	293.15	0	337.238	337.238	0.0765813	0.0765543

636	63.91	11.093	19.9956	0.0149427	0.46834	293.15	293.15	0	337.065	337.065	0.0765428	0.0765155

637	63.74	11.0437	19.9946	0.0148771	0.468113	293.15	293.15	0	336.908	336.908	0.076503	0.0764759

638	63.58	10.9739	20.0008	0.0147837	0.459647	293.15	293.15	0	336.736	336.736	0.0764646	0.0764372

639	63.41	10.8963	20.0008	0.01468	0.457064	293.15	293.15	0	336.571	336.571	0.076426	0.0763989

640	63.24	10.8227	20.0008	0.0145816	0.452006	293.15	293.15	0	336.39	336.39	0.0763869	0.0763594

641	63.08	10.8274	20.0008	0.0145886	0.448085	293.15	293.15	0	336.241	336.241	0.0763486	0.0763209

642	62.91	10.9149	20.0008	0.0147072	0.443519	293.15	293.15	0	336.062	336.062	0.0763082	0.0762809

643	62.74	10.9976	20.0008	0.0148195	0.440777	293.15	293.15	0	335.895	335.895	0.0762693	0.0762416

644	62.57	10.9168	20.0008	0.0147113	0.43893	293.15	293.15	0	335.729	335.729	0.0762302	0.0762025

645	62.41	10.849	20.0008	0.0146207	0.434731	293.15	293.15	0	335.574	335.574	0.0761926	0.0761641

646	62.24	10.792	19.9987	0.0145446	0.427586	293.15	293.15	0	335.406	335.406	0.0761536	0.0761256

647	62.07	10.7166	19.9977	0.0144438	0.425899	293.15	293.15	0	335.236	335.236	0.0761142	0.0760857

648	61.9	10.7321	20.0008	0.0144654	0.423499	293.15	293.15	0	335.06	335.06	0.0760746	0.076046

649	61.74	10.8193	20.0008	0.0145836	0.419072	293.15	293.15	0	334.907	334.907	0.0760356	0.076007

650	61.56	10.9436	20.0008	0.014752	0.417339	293.15	293.15	0	334.733	334.733	0.0759954	0.0759662

651	61.4	11.0281	20.0008	0.0148666	0.41203	293.15	293.15	0	334.568	334.568	0.0759573	0.0759283

652	61.23	11.0189	20.0008	0.014855	0.408887	293.15	293.15	0	334.406	334.406	0.0759183	0.075889

653	61.07	10.9046	20.0008	0.0147015	0.407211	293.15	293.15	0	334.24	334.24	0.0758797	0.0758504

654	60.9	10.8545	20.0008	0.0146348	0.399715	293.15	293.15	0	334.075	334.075	0.0758408	0.0758112

655	60.73	10.9268	20.0008	0.0147331	0.397819	293.15	293.15	0	333.903	333.903	0.0758018	0.075772

656	60.57	10.9934	19.9966	0.0148236	0.393333	293.15	293.15	0	333.738	333.738	0.0757631	0.0757327

657	60.4	11.0234	19.9946	0.0148648	0.392043	293.15	293.15	0	333.566	333.566	0.0757236	0.0756935

658	60.23	11.0317	20.0008	0.0148767	0.387212	293.15	293.15	0	333.397	333.397	0.0756849	0.0756545

659	60.06	11.0023	20.0008	0.0148378	0.384813	293.15	293.15	0	333.237	333.237	0.0756443	0.0756147

660	59.9	10.9301	20.0008	0.0147412	0.379434	293.15	293.15	0	333.069	333.069	0.075606	0.0755762

661	59.73	10.8561	20.0081	0.0146422	0.374404	293.15	293.15	0	332.913	332.913	0.075568	0.0755375

662	59.56	10.817	20.0091	0.0145902	0.372663	293.15	293.15	0	332.745	332.745	0.0755281	0.0754975

663	59.39	10.8434	20.0008	0.0146265	0.369419	293.15	293.15	0	332.576	332.576	0.0754894	0.0754587

664	59.23	10.8396	20.0008	0.014622	0.36525	293.15	293.15	0	332.398	332.398	0.0754499	0.0754197

665	59.06	10.8134	20.0008	0.0145875	0.362178	293.15	293.15	0	332.229	332.229	0.0754109	0.0753798

666	58.89	10.8128	19.9998	0.0145874	0.357116	293.15	293.15	0	332.063	332.063	0.0753728	0.0753416

667	58.72	10.8418	19.9966	0.0146273	0.3533	293.15	293.15	0	331.908	331.908	0.0753329	0.0753011

668	58.55	10.848	20.0008	0.0146364	0.351635	293.15	293.15	0	331.743	331.743	0.0752939	0.075262

669	58.39	10.8478	20.0008	0.0146369	0.346684	293.15	293.15	0	331.562	331.562	0.0752549	0.0752233

670	58.22	10.803	20.0008	0.0145772	0.342597	293.15	293.15	0	331.405	331.405	0.0752162	0.0751847

671	58.06	10.7601	20.0008	0.01452	0.342537	293.15	293.15	0	331.249	331.249	0.0751766	0.0751451

672	57.89	10.7634	19.9956	0.0145252	0.33534	293.15	293.15	0	331.067	331.067	0.0751377	0.0751059

673	57.72	10.8514	19.9956	0.0146448	0.333702	293.15	293.15	0	330.904	330.904	0.0750987	0.0750659

674	57.55	10.9088	20.0008	0.014723	0.328918	293.15	293.15	0	330.73	330.73	0.0750594	0.0750268

675	57.39	11.7191	20.005	0.0158173	0.309051	293.15	293.15	0	330.573	330.573	0.0750283	0.0749891

676	57.26	15.3732	20.0112	0.0207501	0.262629	293.15	293.15	0	330.4	330.4	0.0750099	0.0749579

677	57.13	20.9539	20.0112	0.0282838	0.220286	293.15	293.15	0	330.237	330.237	0.0749897	0.0749284

678	56.99	26.4726	20.005	0.0357344	0.184445	293.15	293.15	0	330.064	330.064	0.0749634	0.0748955

679	56.83	31.8496	20.0081	0.0429949	0.157152	293.15	293.15	0	329.906	329.906	0.0749321	0.0748574

680	56.66	36.8973	20.0008	0.0498114	0.127422	293.15	293.15	0	329.737	329.737	0.0748992	0.0748182

681	56.49	41.7965	20.0008	0.0564284	0.0984238	293.15	293.15	0	329.577	329.577	0.0748665	0.0747779

682	56.31	46.852	20.0008	0.0632569	0.0721165	293.15	293.15	0	329.409	329.409	0.074832	0.0747366

683	56.13	51.9058	19.9935	0.0700842	0.0457548	293.15	293.15	0	329.23	329.23	0.0747969	0.0746946

684	55.94	57.0753	19.9914	0.0770685	0.0219251	293.15	293.15	0	329.071	329.071	0.0747598	0.0746504

685	55.75	62.1345	20.0008	0.0839049	0.00123946	293.15	293.15	0	328.91	328.91	0.0747202	0.0746042

686	55.55	66.9799	20.0008	0.0904534	-0.022246	293.15	293.15	0	328.734	328.734	0.0746815	0.0745588

687	55.38	71.8873	20.0008	0.0970856	-0.0546703	293.15	293.15	0	328.562	328.562	0.0746477	0.0745178

688	55.23	76.7112	20.0008	0.103605	-0.0941154	293.15	293.15	0	328.397	328.397	0.0746175	0.0744822

689	55.09	81.1272	19.9904	0.109574	-0.136806	293.15	293.15	0	328.242	328.242	0.0745899	0.0744497

690	54.96	84.9659	19.9904	0.114763	-0.19026	293.15	293.15	0	328.069	328.069	0.0745643	0.0744196

691	54.84	88.0841	19.9904	0.118979	-0.244297	293.15	293.15	0	327.896	327.896	0.0745373	0.0743915

692	54.72	90.1059	20.0008	0.121715	-0.293509	293.15	293.15	0	327.729	327.729	0.0745091	0.0743632

693	54.6	90.9809	20.005	0.122901	-0.342534	293.15	293.15	0	327.568	327.568	0.0744797	0.0743341

694	54.47	91.0114	19.9925	0.122947	-0.389535	293.15	293.15	0	327.402	327.402	0.0744464	0.0743039

695	54.34	90.4232	19.9935	0.122158	-0.431878	293.15	293.15	0	327.245	327.245	0.0744132	0.0742729

696	54.19	89.2571	20.0008	0.120587	-0.475185	293.15	293.15	0	327.075	327.075	0.0743765	0.0742396

697	54.05	88.1669	20.0008	0.11912	-0.5348	293.15	293.15	0	326.899	326.899	0.0743455	0.0742062

698	53.93	88.8324	20.0008	0.120023	-0.596526	293.15	293.15	0	326.739	326.739	0.0743203	0.0741776

699	53.81	88.8898	20.0008	0.120105	-0.647794	293.15	293.15	0	326.578	326.578	0.0742868	0.0741487

700	53.67	87.4952	20.0008	0.118226	-0.695785	293.15	293.15	0	326.401	326.401	0.0742505	0.074116

701	53.52	85.3872	20.0008	0.115383	-0.733878	293.15	293.15	0	326.248	326.248	0.0742107	0.0740806

702	53.36	82.9936	20.0008	0.112154	-0.780196	293.15	293.15	0	326.073	326.073	0.0741706	0.0740439

703	53.19	80.4384	20.0008	0.108706	-0.81518	293.15	293.15	0	325.902	325.902	0.0741275	0.0740041

704	53.01	77.8308	20.0008	0.105188	-0.847435	293.15	293.15	0	325.728	325.728	0.0740826	0.0739624

705	52.83	75.1747	20.0008	0.101604	-0.873188	293.15	293.15	0	325.581	325.581	0.0740362	0.0739204

706	52.65	72.5183	20.0008	0.098019	-0.900488	293.15	293.15	0	325.398	325.398	0.0739892	0.0738775

707	52.45	69.8297	20.0008	0.0943906	-0.921481	293.15	293.15	0	325.234	325.234	0.0739408	0.0738314

708	52.26	67.2909	20.0008	0.0909643	-0.942201	293.15	293.15	0	325.06	325.06	0.0738918	0.0737851

709	52.05	64.8308	20.0008	0.0876442	-0.953168	293.15	293.15	0	324.905	324.905	0.0738412	0.0737371

710	51.84	62.4476	20.0008	0.0844278	-0.961362	293.15	293.15	0	324.733	324.733	0.0737882	0.0736878

711	51.63	60.1952	20.0008	0.0813877	-0.969348	293.15	293.15	0	324.565	324.565	0.0737373	0.0736381

712	51.42	57.9228	20.0008	0.0783204	-0.970127	293.15	293.15	0	324.405	324.405	0.0736834	0.0735879

713	51.2	55.6747	20.0008	0.0752856	-0.970079	293.15	293.15	0	324.236	324.236	0.0736297	0.0735365

714	50.98	53.5405	20.0008	0.0724044	-0.962901	293.15	293.15	0	324.068	324.068	0.0735761	0.0734851

715	50.75	51.5107	20.0008	0.0696644	-0.947992	293.15	293.15	0	323.899	323.899	0.0735191	0.0734317

716	50.53	49.5406	20.0008	0.0670045	-0.938066	293.15	293.15	0	323.731	323.731	0.0734646	0.0733789

717	50.29	47.5639	19.9946	0.0643356	-0.918404	293.15	293.15	0	323.568	323.568	0.0734081	0.0733241

718	50.07	45.6647	19.9904	0.0617709	-0.896114	293.15	293.15	0	323.402	323.402	0.0733518	0.0732702

719	49.83	43.8356	20.0008	0.059301	-0.866725	293.15	293.15	0	323.237	323.237	0.0732932	0.0732142

720	49.59	42.0672	20.0008	0.0569128	-0.833152	293.15	293.15	0	323.072	323.072	0.0732357	0.0731585

721	49.36	40.2701	20.0008	0.0544854	-0.795334	293.15	293.15	0	322.901	322.901	0.0731783	0.0731034

722	49.12	38.445	20.0008	0.0520198	-0.76177	293.15	293.15	0	322.735	322.735	0.0731198	0.0730478

723	48.88	36.6078	20.0008	0.0495375	-0.716806	293.15	293.15	0	322.578	322.578	0.0730614	0.0729908

724	48.63	34.7786	20.0008	0.0470657	-0.663401	293.15	293.15	0	322.408	322.408	0.0730014	0.0729323

725	48.38	32.9274	20.0008	0.0445639	-0.610514	293.15	293.15	0	322.232	322.232	0.072941	0.0728748

726	48.14	31.1305	20.0008	0.0421351	-0.551291	293.15	293.15	0	322.063	322.063	0.072881	0.0728163

727	47.88	29.414	20.0008	0.0398149	-0.49068	293.15	293.15	0	321.911	321.911	0.0728196	0.0727568

728	47.63	27.7043	19.9935	0.0375035	-0.414664	293.15	293.15	0	321.734	321.734	0.0727589	0.0726981

729	47.38	25.9166	19.9925	0.0350862	-0.336356	293.15	293.15	0	321.565	321.565	0.0726961	0.0726383

730	47.13	24.2475	20.0008	0.032829	-0.264509	293.15	293.15	0	321.401	321.401	0.072635	0.0725787

731	46.87	22.7303	20.0008	0.0307773	-0.186835	293.15	293.15	0	321.244	321.244	0.0725753	0.0725195

732	46.62	21.3068	20.0008	0.0288521	-0.0976047	293.15	293.15	0	321.078	321.078	0.0725121	0.0724595

733	46.37	20.1599	19.9946	0.0273012	-0.00469106	293.15	293.15	0	320.898	320.898	0.072453	0.0724005

734	46.12	19.2003	19.9904	0.0260036	0.0791652	293.15	293.15	0	320.732	320.732	0.0723955	0.0723423

735	45.92	18.4295	19.9904	0.0249612	0.145886	293.15	293.15	0	320.577	320.577	0.0723476	0.0722953

736	45.8	17.4953	20.0008	0.0236968	0.192338	293.15	293.15	0	320.403	320.403	0.0723151	0.0722656

737	45.71	16.0054	20.0008	0.0216792	0.220789	293.15	293.15	0	320.24	320.24	0.072292	0.0722459

738	45.65	14.1017	20.0008	0.0191011	0.234083	293.15	293.15	0	320.067	320.067	0.0722752	0.072232

739	45.61	12.0205	20.0008	0.0162823	0.237262	293.15	293.15	0	319.91	319.91	0.072261	0.0722208

740	45.55	10.1027	20.0008	0.0136847	0.23686	293.15	293.15	0	319.729	319.729	0.0722471	0.0722089

741	45.5	8.4825	20.0008	0.0114903	0.231149	293.15	293.15	0	319.579	319.579	0.0722335	0.0721971

742	45.45	7.16529	20.0008	0.00970614	0.218242	293.15	293.15	0	319.4	319.4	0.0722207	0.072185

743	45.39	6.19159	20.0008	0.00838733	0.203708	293.15	293.15	0	319.233	319.233	0.0722056	0.0721697

744	45.32	5.55549	20.0008	0.00752581	0.192014	293.15	293.15	0	319.064	319.064	0.0721874	0.0721525

745	45.23	5.18487	19.9935	0.00702393	0.180318	293.15	293.15	0	318.903	318.903	0.0721671	0.0721319

746	45.13	5.0468	19.9925	0.00683708	0.166778	293.15	293.15	0	318.726	318.726	0.072146	0.0721099

747	45.03	5.1047	20.0008	0.00691574	0.153937	293.15	293.15	0	318.574	318.574	0.0721221	0.0720858

748	44.92	5.24718	20.0008	0.00710901	0.141988	293.15	293.15	0	318.409	318.409	0.0720962	0.072059

749	44.8	5.48075	20.0008	0.00742574	0.130208	293.15	293.15	0	318.237	318.237	0.0720687	0.0720304

750	44.67	5.7737	20.0008	0.00782295	0.121093	293.15	293.15	0	318.079	318.079	0.0720391	0.072

751	44.54	6.16382	19.9956	0.00835188	0.106163	293.15	293.15	0	317.915	317.915	0.0720094	0.071969

752	44.39	6.64888	19.9904	0.00900953	0.100746	293.15	293.15	0	317.743	317.743	0.0719754	0.0719344

753	44.24	7.13943	20.006	0.00967466	0.0908416	293.15	293.15	0	317.569	317.569	0.0719421	0.0719004

754	44.09	7.58089	20.0071	0.0102734	0.0850763	293.15	293.15	0	317.404	317.404	0.0719076	0.0718647

755	43.94	7.94902	20.0008	0.0107727	0.0801847	293.15	293.15	0	317.239	317.239	0.0718719	0.0718292

756	43.79	8.28832	20.0008	0.0112331	0.0754213	293.15	293.15	0	317.068	317.068	0.0718367	0.0717932

757	43.63	8.56976	20.0008	0.0116151	0.0675658	293.15	293.15	0	316.902	316.902	0.0717987	0.0717553

758	43.47	8.80891	20.0008	0.0119398	0.0610508	293.15	293.15	0	316.73	316.73	0.0717611	0.0717181

759	43.31	9.02884	20.0008	0.0122385	0.0584335	293.15	293.15	0	316.571	316.571	0.0717236	0.0716793

760	43.14	9.23402	19.9977	0.0125172	0.050948	293.15	293.15	0	316.399	316.399	0.0716857	0.0716407

761	42.98	9.45908	19.9987	0.012823	0.0463241	293.15	293.15	0	316.229	316.229	0.071648	0.0716029

762	42.82	9.69986	20.0008	0.01315	0.0460071	293.15	293.15	0	316.077	316.077	0.071608	0.0715635

763	42.65	9.87534	20.0008	0.0133886	0.0428361	293.15	293.15	0	315.904	315.904	0.0715694	0.0715241

764	42.48	9.97864	20.0008	0.0135293	0.041558	293.15	293.15	0	315.737	315.737	0.07153	0.0714848

765	42.31	10.0278	19.9998	0.0135967	0.0374213	293.15	293.15	0	315.575	315.575	0.0714903	0.0714449

766	42.14	10.0993	19.9914	0.0136943	0.0357308	293.15	293.15	0	315.409	315.409	0.0714508	0.0714047

767	41.97	10.1866	20.0008	0.0138135	0.0320775	293.15	293.15	0	315.237	315.237	0.0714123	0.0713651

768	41.81	10.2706	20.0008	0.013928	0.0276497	293.15	293.15	0	315.072	315.072	0.0713733	0.0713266

769	41.63	10.3601	20.0008	0.0140502	0.0298979	293.15	293.15	0	314.907	314.907	0.0713327	0.071285

770	41.47	10.4402	20.0008	0.0141595	0.0277646	293.15	293.15	0	314.735	314.735	0.0712919	0.0712453

771	41.3	10.4836	20.0008	0.0142191	0.0223058	293.15	293.15	0	314.569	314.569	0.0712535	0.0712067

772	41.13	10.4321	20.0008	0.01415	0.0214492	293.15	293.15	0	314.397	314.397	0.0712146	0.0711664

773	40.96	10.427	20.0008	0.0141438	0.0220014	293.15	293.15	0	314.24	314.24	0.0711745	0.0711263

774	40.79	10.4615	20.0008	0.0141914	0.0181124	293.15	293.15	0	314.067	314.067	0.0711347	0.0710863

775	40.63	10.4583	20.0008	0.0141877	0.0144159	293.15	293.15	0	313.896	313.896	0.0710953	0.0710469

776	40.46	10.4193	20.0008	0.0141355	0.0164335	293.15	293.15	0	313.739	313.739	0.0710556	0.0710077

777	40.29	10.4024	19.9977	0.0141133	0.0121744	293.15	293.15	0	313.572	313.572	0.0710161	0.0709685

778	40.13	10.3907	19.9987	0.0140981	0.00407387	293.15	293.15	0	313.404	313.404	0.0709786	0.0709303

779	39.97	10.3675	20.0008	0.0140673	0.00153726	293.15	293.15	0	313.243	313.243	0.0709394	0.0708914

780	39.8	10.3431	20.0008	0.014035	-0.0025716	293.15	293.15	0	313.066	313.066	0.0709013	0.0708532

781	39.65	10.341	20.0008	0.0140327	-0.00912215	293.15	293.15	0	312.913	312.913	0.0708652	0.0708168

782	39.5	10.2863	20.0008	0.0139591	-0.0186984	293.15	293.15	0	312.748	312.748	0.0708289	0.0707805

783	39.35	10.1882	20.0008	0.0138267	-0.0324197	293.15	293.15	0	312.567	312.567	0.0707937	0.0707453

784	39.2	10.0799	20.0008	0.0136803	-0.0416074	293.15	293.15	0	312.411	312.411	0.0707574	0.0707095

785	39.04	9.90898	20.0008	0.013449	-0.0526289	293.15	293.15	0	312.246	312.246	0.0707219	0.0706739

786	38.9	9.75705	20.0008	0.0132434	-0.069857	293.15	293.15	0	312.073	312.073	0.0706874	0.0706392

787	38.76	9.62023	20.0008	0.0130582	-0.0887849	293.15	293.15	0	311.899	311.899	0.070653	0.0706055

788	38.61	9.5338	20.0008	0.0129415	-0.10927	293.15	293.15	0	311.726	311.726	0.07062	0.0705718

789	38.47	9.40269	19.9956	0.012764	-0.125895	293.15	293.15	0	311.578	311.578	0.0705867	0.0705385

790	38.33	9.27359	20.0008	0.0125893	-0.149244	293.15	293.15	0	311.398	311.398	0.0705542	0.070506

791	38.2	9.18153	20.0008	0.0124649	-0.172861	293.15	293.15	0	311.233	311.233	0.0705216	0.0704738

792	38.06	9.12425	20.0008	0.0123876	-0.202957	293.15	293.15	0	311.066	311.066	0.0704903	0.0704416

793	37.93	9.05491	20.0008	0.012294	-0.22824	293.15	293.15	0	310.912	310.912	0.0704587	0.0704102

794	37.8	8.9295	20.0039	0.0121242	-0.261117	293.15	293.15	0	310.742	310.742	0.0704277	0.0703798

795	37.67	8.73509	20.0091	0.0118607	-0.296424	293.15	293.15	0	310.578	310.578	0.0703975	0.0703496

796	37.54	8.51036	20.0008	0.011556	-0.333324	293.15	293.15	0	310.409	310.409	0.0703675	0.0703195

797	37.42	8.34907	20.0008	0.0113374	-0.37549	293.15	293.15	0	310.235	310.235	0.0703376	0.0702903

798	37.3	8.24423	19.9935	0.0111955	-0.418093	293.15	293.15	0	310.067	310.067	0.0703092	0.0702612

799	37.18	8.18144	19.9914	0.0111106	-0.457765	293.15	293.15	0	309.914	309.914	0.0702801	0.0702323

800	37.05	8.11125	20.0008	0.0110157	-0.508897	293.15	293.15	0	309.74	309.74	0.0702515	0.0702035

801	36.94	7.97368	20.0008	0.0108292	-0.5604	293.15	293.15	0	309.569	309.569	0.0702234	0.0701759

802	36.82	7.87258	20.0008	0.0106923	-0.613072	293.15	293.15	0	309.403	309.403	0.0701959	0.070148

803	36.7	7.77065	20.0008	0.0105543	-0.663441	293.15	293.15	0	309.247	309.247	0.0701684	0.070121

804	36.59	7.63133	19.9956	0.0103654	-0.728485	293.15	293.15	0	309.065	309.065	0.0701416	0.0700943

805	36.48	7.51653	19.9904	0.0102098	-0.7906	293.15	293.15	0	308.901	308.901	0.0701145	0.0700673

806	36.37	7.41782	20.0008	0.0100761	-0.857961	293.15	293.15	0	308.728	308.728	0.0700883	0.0700417

807	36.26	7.31868	20.0008	0.00994172	-0.922904	293.15	293.15	0	308.571	308.571	0.070063	0.0700163

808	36.15	7.23892	20.0008	0.00983369	-0.998664	293.15	293.15	0	308.398	308.398	0.0700382	0.0699909

809	36.04	7.11272	20.006	0.00966259	-1.06624	293.15	293.15	0	308.245	308.245	0.0700123	0.0699648

810	35.94	6.91029	20.0039	0.00938788	-1.14537	293.15	293.15	0	308.077	308.077	0.0699874	0.0699405

811	35.84	6.77154	20.0029	0.00919967	-1.23212	293.15	293.15	0	307.903	307.903	0.0699634	0.0699166

812	35.74	6.68524	20.0008	0.00908271	-1.31929	293.15	293.15	0	307.734	307.734	0.0699397	0.0698925

813	35.64	6.59539	20.0008	0.0089609	-1.40394	293.15	293.15	0	307.574	307.574	0.0699157	0.0698692

814	35.54	6.52251	20.0008	0.00886215	-1.49976	293.15	293.15	0	307.406	307.406	0.0698925	0.0698456

815	35.44	6.47548	20.0008	0.00879852	-1.59714	293.15	293.15	0	307.236	307.236	0.0698694	0.0698225

816	35.35	6.37894	20.0008	0.0086676	-1.70107	293.15	293.15	0	307.064	307.064	0.0698468	0.0697998

817	35.25	6.31591	20.0008	0.00858219	-1.80607	293.15	293.15	0	306.896	306.896	0.0698244	0.0697778

818	35.16	6.26227	19.9998	0.00850955	-1.91025	293.15	293.15	0	306.736	306.736	0.0698022	0.0697559

819	35.07	6.22917	19.9914	0.00846481	-2.02126	293.15	293.15	0	306.57	306.57	0.0697803	0.0697341

820	34.98	6.16336	20.0008	0.00837561	-2.13681	293.15	293.15	0	306.404	306.404	0.0697585	0.0697121

821	34.89	6.06799	20.0008	0.00824623	-2.26233	293.15	293.15	0	306.232	306.232	0.0697379	0.0696918

822	34.8	5.96003	19.9946	0.00809973	-2.38554	293.15	293.15	0	306.066	306.066	0.0697173	0.069671

823	34.71	5.83166	19.9956	0.0079255	-2.50431	293.15	293.15	0	305.912	305.912	0.0696968	0.06965

824	34.63	5.73476	20.0008	0.007794	-2.64209	293.15	293.15	0	305.738	305.738	0.0696763	0.0696298

825	34.54	5.69248	20.0008	0.00773674	-2.78236	293.15	293.15	0	305.565	305.565	0.0696559	0.0696102

826	34.46	5.6168	20.0008	0.00763407	-2.9234	293.15	293.15	0	305.399	305.399	0.069637	0.0695911

827	34.38	5.53321	20.0008	0.00752065	-3.06701	293.15	293.15	0	305.237	305.237	0.0696176	0.0695712

828	34.3	5.48478	20.0008	0.00745502	-3.21488	293.15	293.15	0	305.071	305.071	0.0695982	0.0695515

829	34.22	5.4376	20.0008	0.00739106	-3.35915	293.15	293.15	0	304.914	304.914	0.0695796	0.069533

830	34.14	5.36322	20.0008	0.00729014	-3.519	293.15	293.15	0	304.745	304.745	0.06956	0.069514

831	34.06	5.3033	20.0008	0.00720887	-3.68966	293.15	293.15	0	304.572	304.572	0.0695419	0.0694951

832	33.98	5.26732	20.0008	0.00716014	-3.86275	293.15	293.15	0	304.399	304.399	0.0695233	0.0694765

833	33.91	5.15675	20.0008	0.00700998	-4.03777	293.15	293.15	0	304.229	304.229	0.0695059	0.0694593

834	33.83	5.02558	20.0008	0.00683182	-4.21498	293.15	293.15	0	304.063	304.063	0.0694886	0.0694422

835	33.76	4.89849	20.0008	0.00665921	-4.38456	293.15	293.15	0	303.908	303.908	0.0694714	0.0694252

836	33.69	4.76675	20.0008	0.00648025	-4.5697	293.15	293.15	0	303.742	303.742	0.0694546	0.0694087

837	33.62	4.66791	20.0008	0.00634603	-4.77578	293.15	293.15	0	303.561	303.561	0.0694371	0.0693912

838	33.55	4.5911	20.0008	0.00624173	-4.95843	293.15	293.15	0	303.405	303.405	0.0694199	0.0693744

839	33.47	4.59916	20.0008	0.00625283	-5.15452	293.15	293.15	0	303.24	303.24	0.0694034	0.0693571


