Analysis of the specific pentosan content

The specific content of pentosans in wood was estimated using the modified Tollens method [55, 56] by converting them to furfural during distillation in the presence of HCl. For this analysis, two 10 cm long cuts of stem per plant, representing the 1st and the 2nd year growing wood, respectively, were taken from 18-month-old plants. The cuts were stripped off their bark, and the air-dried sawdust samples weighing 0.1 g were prepared. The optical absorption of the distillate was measured by a two-beam spectrophotometer at a wavelength of 277 nm. The dryness coefficient of wood (Сdry) was calculated from the following formulas: W=m1- m2m1-m and Сdry=100 - W100 , where W – the relative humidity of the wood, m – the mass of the empty bag (g), m1 and m2 – the weights (g) of the bag with the sample before and after drying, respectively. Then, the content of pentosans in dry matter was calculated according to the formula: A=D×nm ×Сdry , where A – the percentage of pentosans in the air-dry sample, D – the average optical absorption of the furfural solution obtained from the distillation, n – the conversion factor for the percentage of furfural to pentosans (2.434 for hardwoods), m – the mass of the sawdust sample (g), Сdry – coefficient of dryness. For clarity, the percentage of pentosans was converted to absolute values as mg / g dry weight.