APPENDIX 1

REBOUND HAMMER TEST RESULTS

| Block A Last floor beam-spall Angle = +90 Degree |  |  |  |  | Block A Last floor s30lab (Toilet)--damp Angle = +90 Degree |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| S/N | Rebound value | Compressive strength value (MPa) |  |  | S/N | Rebound value | Compressive strength value (MPa) |
| 1 | 28 | 14.00 |  |  | 1 | 40 | 32.00 |
| 2 | 25 | 10.00 |  |  | 2 | 40 | 32.00 |
| 3 | 30 | 16.00 |  |  | 3 | 38 | 29.00 |
| 4 | 29 | 15.00 |  |  | 4 | 39 | 30.00 |
| 5 | 28 | 14.00 |  |  | 5 | 40 | 32.00 |
| 6 | 25 | 10.00 |  |  | 6 | 38 | 29.00 |
| 7 | 30 | 16.00 |  |  | 7 | 37 | 27.00 |
| 8 | 30 | 16.00 |  |  | 8 | 39 | 30.00 |
| 9 | 26 | 11.00 |  |  | 9 | 41 | 34.00 |
| 10 | 27 | 12.00 |  |  | 10 | 40 | 32.00 |
| 24 | AVERAGE | 13.40 |  |  | 32 | AVERAGE | 30.70 |

| Block A First-floor Stair wall--damp algae Angle = 0 Degree |  |  |  | Block A First-floor Slab (Toilet )--damp Angle = +90 Degree |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| S/N | Rebound value | Compressive strength value (MPa) |  | S/N | Rebound value | Compressive strength value (MPa) |
| 1 | 20 | 10.00 |  | 1 | 40 | 32.00 |
| 2 | 25 | 16.00 |  | 2 | 39 | 30.00 |
| 3 | 23 | 13.50 |  | 3 | 37 | 27.00 |
| 4 | 29 | 22.00 |  | 4 | 40 | 32.00 |
| 5 | 28 | 20.00 |  | 5 | 40 | 32.00 |
| 6 | 25 | 16.00 |  | 6 | 38 | 29.00 |
| 7 | 26 | 17.00 |  | 7 | 37 | 27.00 |
| 8 | 30 | 23.00 |  | 8 | 38 | 29.00 |
| 9 | 26 | 17.00 |  | 9 | 40 | 32.00 |
| 10 | 27 | 18.00 |  | 10 | 41 | 34.00 |
| 30 | AVERAGE | 17.25 |  | 32 | AVERAGE | 30.40 |

| Block A Ground floor column-mild damp Angle = 0 Degree |  |  |
| --- | --- | --- |
| S/N | Rebound Value | Compressive strength Value (MPa) |
| 1 | 30 | 23.00 |
| 2 | 29 | 22.00 |
| 3 | 30 | 23.00 |
| 4 | 29 | 22.00 |
| 5 | 30 | 23.00 |
| 6 | 30 | 23.00 |
| 7 | 30 | 23.00 |
| 8 | 30 | 23.00 |
| 9 | 29 | 22.00 |
| 10 | 27 | 18.00 |
| 26 | AVERAGE | 22.20 |

| Block B Second-floor column-damp mould Angle = 0 Degree |  |  |  | Block B Second-floor Slab (Toilet)-damp Angle = +90 Degree |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| S/N | Rebound value | Compressive strength value (MPa) |  | S/N | Rebound value | Compressive strength value (MPa) |
| 1 | 32 | 26.00 |  | 1 | 39 | 30.00 |
| 2 | 32 | 26.00 |  | 2 | 40 | 32.00 |
| 3 | 32 | 26.50 |  | 3 | 37 | 27.00 |
| 4 | 34 | 29.70 |  | 4 | 37 | 27.00 |
| 5 | 34 | 29.70 |  | 5 | 40 | 32.00 |
| 6 | 32 | 26.00 |  | 6 | 38 | 29.00 |
| 7 | 30 | 23.00 |  | 7 | 40 | 32.00 |
| 8 | 33 | 28.00 |  | 8 | 35 | 24.00 |
| 9 | 30 | 23.00 |  | 9 | 40 | 32.00 |
| 10 | 32 | 26.00 |  | 10 | 41 | 34.00 |
| 27 | AVERAGE | 26.39 |  | 32 | AVERAGE | 29.90 |
| Block B First-floor Column-damp mould Angle = 0 Degree |  |  |  | Block B First-floor Slab (Toilet)-seru seep Angle = +90 Degree |  |  |
| S/N | Rebound value | Compressive strength value (MPa) |  | S/N | Rebound value | Compressive strength value (MPa) |
| 1 | 32 | 26.00 |  | 1 | 37 | 27.00 |
| 2 | 34 | 29.70 |  | 2 | 37 | 27.00 |
| 3 | 32 | 26.00 |  | 3 | 38 | 29.00 |
| 4 | 32 | 26.00 |  | 4 | 38 | 29.00 |
| 5 | 34 | 29.70 |  | 5 | 28 | 14.00 |
| 6 | 32 | 26.00 |  | 6 | 35 | 24.00 |
| 7 | 30 | 23.00 |  | 7 | 35 | 24.00 |
| 8 | 32 | 26.00 |  | 8 | 28 | 14.00 |
| 9 | 30 | 23.00 |  | 9 | 37 | 27.00 |
| 10 | 30 | 23.00 |  | 10 | 30 | 16.00 |
| 27 | AVERAGE | 25.84 |  | 34 | AVERAGE | 23.10 |

| Block C Ground floor column-damp mould Angle = 0 Degree |  |  |  | Block C Ground floor beam--spall Angle = +90 Degree |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| S/N | Rebound value | Compressive strength value (MPa) |  | S/N | Rebound value | Compressive strength value (MPa) |
| 1 | 32 | 26.00 |  | 1 | 28 | 14.00 |
| 2 | 34 | 29.70 |  | 2 | 28 | 14.00 |
| 3 | 30 | 23.00 |  | 3 | 34 | 22.00 |
| 4 | 30 | 23.00 |  | 4 | 32 | 20.00 |
| 5 | 34 | 29.70 |  | 5 | 32 | 20.00 |
| 6 | 32 | 26.00 |  | 6 | 30 | 16.00 |
| 7 | 30 | 23.00 |  | 7 | 30 | 16.00 |
| 8 | 31 | 24.00 |  | 8 | 28 | 14.00 |
| 9 | 29 | 22.00 |  | 9 | 28 | 14.00 |
| 10 | 29 | 22.00 |  | 10 | 30 | 16.00 |
| 27 | AVERAGE | 24.84 |  | 30 | AVERAGE | 16.60 |

| Block C Second-floor Slab (Toilet) damp Angle = +90 Degree |  |  |
| --- | --- | --- |
| S/N | Rebound Value | Compressive strength Value (MPa) |
| 1 | 40 | 32 |
| 2 | 39 | 30 |
| 3 | 37 | 27 |
| 4 | 40 | 32 |
| 5 | 45 | 42 |
| 6 | 38 | 29 |
| 7 | 37 | 27 |
| 8 | 41 | 34 |
| 9 | 40 | 32 |
| 10 | 35 | 24 |
| 32 | AVERAGE | 30.90 |

| Block D Ground Floor Slab-damp seep crk Angle = +90 Degree |  |  |  |  | Block D Ground Floor Column -damp Angle = 0 Degree |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| S/N | Rebound Value | Compressive strength Value (MPa) |  |  | S/N | Rebound Value | Compressive strength Value (MPa) |
| 1 | 35 |  | 24.00 |  | 1 | 37 | 34.00 |
| 2 | 37 |  | 27.00 |  | 2 | 38 | 36.00 |
| 3 | 38 |  | 29.00 |  | 3 | 33 | 28.00 |
| 4 | 39 |  | 31.00 |  | 4 | 39 | 38.00 |
| 5 | 32 |  | 20.00 |  | 5 | 35 | 31.00 |
| 6 | 35 |  | 24.00 |  | 6 | 35 | 31.00 |
| 7 | 37 |  | 27.00 |  | 7 | 37 | 34.00 |
| 8 | 35 |  | 24.00 |  | 8 | 39 | 38.00 |
| 9 | 35 |  | 24.00 |  | 9 | 36 | 33.00 |
| 10 | 32 |  | 20.00 |  | 10 | 33 | 28.00 |
| 33 | AVERAGE |  | 25.00 |  | 35 | AVERAGE | 33.1 |

| Block D First floor Slab(Toilet )-spalling Angle = +90 Degree |  |  |  | Block D Second floor slab- crack Angle = +90 Degree |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| S/N | Rebound value | Compressive strength value (MPa) |  | S/N | Rebound value | Compressive strength value (MPa) |
| 1 | 35 | 24.00 |  | 1 | 34 | 22.00 |
| 2 | 34 | 22.00 |  | 2 | 32 | 20.00 |
| 3 | 38 | 29.00 |  | 3 | 35 | 24.00 |
| 4 | 37 | 27.00 |  | 4 | 39 | 30.00 |
| 5 | 32 | 20.00 |  | 5 | 40 | 32.00 |
| 6 | 32 | 20.00 |  | 6 | 33 | 21.00 |
| 7 | 33 | 21.00 |  | 7 | 31 | 18.00 |
| 8 | 34 | 22.00 |  | 8 | 39 | 30.00 |
| 9 | 34 | 22.00 |  | 9 | 35 | 24.00 |
| 10 | 32 | 20.00 |  | 10 | 34 | 22.00 |
| 32 | AVERAGE | 22.70 |  | 32 | AVERAGE | 24.30 |

| Block E Ground floor column-damp Angle = 0 Degree |  |  |  | Block E First floor slab(toilet)-damp crack Angle = +90 Degree |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| S/N | Rebound value | Compressive strength value (MPa) |  | S/N | Rebound value | Compressive strength value (MPa) |
| 1 | 30 | 23.00 |  | 1 | 38 | 29.00 |
| 2 | 28 | 20.00 |  | 2 | 32 | 20.00 |
| 3 | 27 | 18.00 |  | 3 | 34 | 22.00 |
| 4 | 32 | 26.00 |  | 4 | 38 | 29.00 |
| 5 | 28 | 20.00 |  | 5 | 37 | 27.00 |
| 6 | 27 | 18.00 |  | 6 | 33 | 21.00 |
| 7 | 30 | 23.00 |  | 7 | 36 | 26.00 |
| 8 | 30 | 23.00 |  | 8 | 35 | 24.00 |
| 9 | 30 | 23.00 |  | 9 | 35 | 24.00 |
| 10 | 32 | 26.00 |  | 10 | 34 | 22.00 |
| 26 | AVERAGE | 22.00 |  | 30 | AVERAGE | 24.40 |

| Block E Second floor Slab(Toilet)-damp Angle = 0 Degree |  |  |  | Block E Second floor Slab-spall Angle = +90 Degree |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| S/N | Rebound value | Compressive strength value (MPa) |  | S/N | Rebound value | Compressive strength value (MPa) |  |
| 1 | 37 | 27.00 |  | 1 | 30 | 16.00 |
| 2 | 38 | 29.00 |  | 2 | 30 | 16.00 |
| 3 | 36 | 26.00 |  | 3 | 32 | 20.00 |
| 4 | 40 | 32.00 |  | 4 | 38 | 29.00 |
| 5 | 38 | 29.00 |  | 5 | 37 | 27.00 |
| 6 | 40 | 32.00 |  | 6 | 33 | 21.00 |
| 7 | 36 | 26.00 |  | 7 | 36 | 26.00 |
| 8 | 38 | 29.00 |  | 8 | 30 | 16.00 |
| 9 | 36 | 26.00 |  | 9 | 30 | 16.00 |
| 10 | 38 | 29.00 |  | 10 | 34 | 22.00 |
| 30 | AVERAGE | 28.50 |  | 30 | AVERAGE | 20.30 |