Combustion and mechanical property enhancement strategy based on SA surface activated boron powders

Jiaxin Lu, Chong Chen, Bobo Zhang, Kang Niu, Fei Xiao, Taixin Liang*

School of Environment and Safety Engineering, North University of China, Taiyuan 030051, Shanxi, China.

Corresponding author: liangtx2006@126.com (Taixin Liang).

Figure S1. State of B and SA@B composite particles in water

Figure S2. The XRD represents the combustion product of B, mechanical mixture SA@B composite particles and SA@B composite particles.

Figure S3. The combustion phenomena of B particle and SA@B composite particle in an oxygen atmosphere at 800℃.

Figure S4. The combustion phenomena of B particle and SA@B composite particle in an oxygen atmosphere at 700℃.

Figure S5. SEM images of the reaction products of (a) B, (b) SA@B at 800℃ in the air atmosphere.

Figure S6. The XRD curves of reaction products of B and SA@B at 800℃ in the air atmosphere.

Table S1. Mechanical property data of B/HTPB and SA@B/HTPB composite materials obtained from stress-strain curves.

| Sample | Tensile strength (MPa) | Elongation (%) | Young’s modulus (MPa) | Toughness (MJ/m3) |
| --- | --- | --- | --- | --- |
| 20 wt% B/HTPB | 0.36 | 465.6 | 0.56 | 0.93 |
| 35 wt% B/HTPB | 0.05 | 96.1 | 0.50 | 0.23 |
| 20 wt% SA@B/HTPB | 0.42 | 302.6 | 2.03 | 2.44 |
| 35 wt% SA@B/HTPB | 0.46 | 112.1 | 5.85 | 1.72 |
| 50 wt% SA@B/HTPB | 0.63 | 88.8 | 7.48 | 1.69 |