Supporting information for

The adsorption/desorption of phenanthrene and ofloxacin by microbial residues-mineral composites: different substrate-C and minerals

Qiuling Yan a, Zhicheng Tan a, Zhongwen Li a, Jiawen Guo b, Yuxuan Li a, Siyao Wang a, Fangfang Li a, *, Lin Wang a, Hongbo Peng c, *

a Yunnan Key Laboratory of Soil Carbon Sequestration and Pollution Control, Faculty of Environmental Science and Engineering, Kunming University of Science and Technology, Kunming 650500, China

b Yunnan Sugarcane Research Institute, Yunnan Academy of Agricultural Sciences, Kaiyuan, China, 661699, China

c Faculty of Modern Agricultural Engineering, Kunming University of Science & Technology, Kunming, Yunnan 650500, China

Table S1. Physicochemical properties of microbial residues-mineral composites including the elemental analysis and specific surface area.

| Name | Elemental analysis |  |  |  |  |  | SSA（m2/g） | Pore volume cm3/g | Pore radius nm |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | N% | C% | H% | O% | C/H | (N+O)/C |  |  |  |
| GF | 0.02 | 0.24 | 0.14 | 4.73 | 0.14 | 14.85 | 1.075 | 0.005 | 19.059 |
| PF | 0.02 | 0.64 | 0.24 | 3.19 | 0.23 | 3.77 | 1.069 | 0.007 | 24.860 |
| BF | 0.01 | 0.98 | 0.35 | 7.08 | 0.24 | 5.43 | 0.953 | 0.006 | 25.259 |
| FQ | 0.01 | 0.04 | 0.06 | 1.14 | - | - | 2.774 | 0.012 | 16.306 |
| GM | 0.20 | 0.64 | 0.73 | 5.54 | 0.07 | 6.76 | 7.649 | 0.034 | 17.150 |
| PM | 0.15 | 1.54 | 0.31 | 5.91 | 0.42 | 2.96 | 8.856 | 0.037 | 16.110 |
| BM | 0.06 | 2.11 | 0.16 | 6.33 | 1.10 | 2.27 | 8.611 | 0.040 | 18.252 |
| MQ | 0.01 | 0 | 0.06 | 0.91 | - | - | 36.363 | 0.073 | 7.801 |

Table S2. Selected physical and chemical properties of PHE

| Name | Molecular formula | Molecular Weight (g/mol) |  | CS a (mg/L) | log KOW a |  | pKa1/ pKa2 | Chemical structure |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PHE | C14H10 | 178.23 | 1.3 |  | 4.74 | - |  |  |
| OFL | C18H20FN3O4 | 361.37 | 3400 |  | -0.35 | 6.10/8.28 |  |  |

a Measured at 25 ºC.

Table S3. The zeta potential of microbial residues-mineral composites measured at adsorption equilibrium pH.

| Name | pH 1 | Zeta potential 1 （mV） |  | pH 2 | Zeta potential 1 （mV） |
| --- | --- | --- | --- | --- | --- |
| GF | 8.96 |  | -25.76 | 9.13 | -36.81 |
| PF | 8.99 |  | -20.55 | 9.21 | -24.40 |
| BF | 9.22 |  | -35.35 | 9.25 | -29.75 |
| FQ | 9.33 |  | -34.40 | 9.57 | -40.85 |
| GM | 9.29 |  | -34.99 | 9.31 | -30.29 |
| PM | 9.37 |  | -10.50 | 9.50 | -20.60 |
| BM | 9.35 |  | -23.13 | 9.38 | -19.07 |
| MQ | 9.30 |  | -27.62 | 9.32 | -25.60 |

Fig S1. The FTIR maps of microbial residues-mineral composites.

* Corresponding author at: Faculty of Environmental Science & Engineering, Kunming University of Science & Technology, Kunming 650500, China.

E-mail address: fangkust@163.com  (F. Li).