For submission to Discover Nano, May 2024.

Preparation Irinotecan Hydrochloride Loaded PEGylated Liposomes Using Novel Method Supercritical Fluid and Condition Optimized by Box-Behnken Design

Misagh Mohammadi1, Mehrnaz Karimi1, Farhad Raofie1*

- Department of Analytical Chemistry and pollutants, Shahid Beheshti University, Tehran

, Iran, 198396941.

* Corresponding author, email: f_raofie@sbu.ac.ir Fax: +98-21-22431661

1https://orcid.org/0000-0001-9227-2107

2 https://orcid.org/0000-0002-1005-5203

3 https://orcid.org/0000-0002-7911-6764

Supplementary material

Figure caption:

Fig. S1: Graphs of the a) size, b) count, c) encapsulation efficiency of nanoliposomes content versus the calculated one during the experimental range of this study.

Fig. S1: Graphs of the a) size, b) count, c) encapsulation efficiency of nanoliposomes content versus the calculated one during the experimental range of this study.

Fig. S2: Counter plots as a function of (a, d, g) flow rate and temperature, (b, e, h) temperature and pressure drop, and (c, f, i) pressure drop and flow rate for the mean size, Count, and EE, respectively.

Fig. S2: Counter plots as a function of (a, d, g) flow rate and temperature, (b, e, h) temperature and pressure drop, and (c, f, i) pressure drop and flow rate for the mean size, Count, and EE, respectively.

Fig. S3: FESEM images of produced irinotecan PEGylated liposomes for experiments 3, 4, 6, 7, 8, 9, 10, 12, and 15, respectively.

Fig. S3: FESEM images of produced irinotecan PEGylated liposomes for experiments 3, 4, 6, 7, 8, 9, 10, 12, and 15, respectively.

Tables

Table S1: coded levels of independent variables used in the RSM design.

| Xi | Independent variables | Units | Coded values |  |  | Response (Y1) | Response (Y2) | Response (Y3) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  | -1 | 0 | 1 |  |  |  |
| A | Flow rate | mL/min | 1.0 | 2.0 | 3.0 | Mean size (nm) | Count | EE (%) |
| B | Pressure drop | MPa | 15.0 | 22.5 | 30.0 |  |  |  |
| C | Temperature | ˚C | 40.0 | 52.5 | 65.0 |  |  |  |

Table S2: ANOVA of predicted second-order polynomial model for mean size of produced irinotecan PEGylated liposomes.

| Source | Sum of Squares | Df | Mean Square | F-Ratio | P-Value |
| --- | --- | --- | --- | --- | --- |
| A: Flow rate | 6.12 | 1 | 6.12 | 1.53 | 0.341 |
| B: Pressure drop | 4050.00 | 1 | 4050.00 | 1012.50 | 0.001 |
| C: Temperature | 300.12 | 1 | 300.12 | 75.03 | 0.013 |
| AA | 33.23 | 1 | 33.23 | 8.31 | 0.102 |
| AB | 30.25 | 1 | 30.25 | 7.56 | 0.111 |
| AC | 100.00 | 1 | 100.00 | 25.00 | 0.038 |
| BB | 600.23 | 1 | 600.23 | 150.06 | 0.007 |
| BC | 6.25 | 1 | 6.25 | 1.56 | 0.338 |
| CC | 887.08 | 1 | 887.08 | 221.77 | 0.004 |
| Lack-of-fit | 193.75 | 3 | 64.58 | 16.15 | 0.059 |
| Pure error | 8.00 | 2 | 4.00 |  |  |
| Total (corr.) | 6081.33 | 14 |  |  |  |

Table S3: ANOVA of predicted second-order polynomial model for count of produced irinotecan PEGylated liposomes.

| Source | Sum of Squares | Df | Mean Square | F-Ratio | P-Value |
| --- | --- | --- | --- | --- | --- |
| A: Flow rate | 84.50 | 1 | 84.50 | 1.03 | 0.418 |
| B: Pressure drop | 313236.00 | 1 | 313236.00 | 3804.49 | 0.001 |
| C: Temperature | 40755.10 | 1 | 40755.10 | 495.00 | 0.002 |
| AA | 46661.60 | 1 | 46661.60 | 566.74 | 0.002 |
| AB | 812.25 | 1 | 812.25 | 9.87 | 0.088 |
| AC | 9120.25 | 1 | 9120.25 | 110.77 | 0.009 |
| BB | 608.10 | 1 | 608.10 | 7.39 | 0.113 |
| BC | 52900.00 | 1 | 52900.00 | 642.51 | 0.002 |
| CC | 21420.40 | 1 | 21420.40 | 260.17 | 0.004 |
| Lack-of-fit | 3983.25 | 3 | 1327.75 | 16.13 | 0.059 |
| Pure error | 164.67 | 2 | 82.33 |  |  |
| Total (corr.) | 487234.00 | 14 |  |  |  |

Table S4: ANOVA of predicted second-order polynomial model for EE of produced irinotecan PEGylated liposomes.

| Source | Sum of Squares | Df | Mean Square | F-Ratio | P-Value |
| --- | --- | --- | --- | --- | --- |
| A: Flow rate | 364.50 | 1 | 364.50 | 364.50 | 0.003 |
| B: Pressure drop | 84.50 | 1 | 84.50 | 84.50 | 0.012 |
| C: Temperature | 84.50 | 1 | 84.50 | 84.50 | 0.012 |
| AA | 48.52 | 1 | 48.51 | 48.52 | 0.020 |
| AB | 132.25 | 1 | 132.25 | 132.25 | 0.007 |
| AC | 0.25 | 1 | 0.25 | 0.25 | 0.667 |
| BB | 48.52 | 1 | 48.51 | 48.52 | 0.020 |
| BC | 12.25 | 1 | 12.25 | 12.25 | 0.073 |
| CC | 96.98 | 1 | 96.98 | 96.98 | 0.010 |
| Lack-of-fit | 10.00 | 3 | 3.33 | 3.33 | 0.239 |
| Pure error | 2 | 2 | 1 |  |  |
| Total (corr.) | 859.60 | 14 |  |  |  |