Support information

Optimized cellulignin production from sugarcane bagasse, sugarcane straw, and energy cane for advanced biofuels: liquor composition and cellulignin characterizations

Igor M. Gonçalvesa, Diego M. Chavesa, Ana B. M. X. Rufinoa, Tales R. Antunesa, Ana J. S. Quintãoa, Renê C. da Silvab, Sukarno O. Ferreirab, Gilmare A. da Silvaa, Luiz A. Peternellic, Márcio H. P. Barbosad, Reinaldo F. Teófiloa*

aChemistry Department, bPhysics Department, cStatistic Department, dAgronomy Departament, Federal University of Viçosa. Av. Peter Henry Rolfs, s/n, Campus Universitário 36570-900 Viçosa/MG, Brazil.

*rteofilo@ufv.br

Table S1: Granulometry of biomasses used in the hydrothermal pretreatment studies

| Sieve set |  | Biomasses (%) |  |  |
| --- | --- | --- | --- | --- |
| Mesh | Aperture (mm) | SCB | EC | SCS |
| > 20 | > 0.850 | 2.21 | 6.14 | 1.63 |
| < 20 and > 35 | < 0.850 and > 0.500 | 53.92 | 61.88 | 70.00 |
| < 35 and > 48 | < 0.500 and > 0.300 | 22.64 | 15.30 | 16.40 |
| < 48 and > 65 | < 0.300 and > 0.212 | 13.21 | 9.48 | 6.21 |
| < 65 and > 80 | < 0.212 and > 0.180 | 2.38 | 2.46 | 1.54 |
| < 80 | < 0.180 | 5.64 | 4.73 | 4.22 |

Table S2: Moisture and ashes content of sugarcane biomasses used in the hydrothermal pretreatment studies

| Experiment | Moisture (%) |  |  | Ashes (%) |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | SCB | EC | SCS | SCB | EC | SCS |
| 1 | 5.42 | 4.36 | 4.32 | 2.05 | 2.94 | 5.62 |
| 2 | 5.39 | 4.09 | 4.53 | 2.22 | 2.86 | 6.07 |
| 3 | 5.75 | 4.27 | 4.76 | 2.15 | 2.99 | 5.72 |
| Average | 5.52 | 4.24 | 4.54 | 2.14 | 2.92 | 5.80 |

Fig. S1: Thermalgravimetric analysis of solid phases from HTP of biomasses: (a) (b) TG and (c) (d) Heat flow curves of SCB pretreated at different temperatures and SCB, SCS and EC treated at 190 ºC and 75 min, respectively, and (e) degradation curves of isolated lignin from untreated SCB. SCB-Sugarcane bagasse, SCS-Sugarcane straw and EC-Energy cane

Fig. S2: Generated solid phases in HTP experiments: (a) biochar produced from pure furfural and (b) selected images of solid phases from HTP of biomasses. SCB-Sugarcane bagasse, SCS-Sugarcane straw and EC-Energy cane