Extended data

Extended Data Figure 1 | Surface chemistry of the probe substrate surface.

FT-IR spectrum of the glass substrate before and after modification with phenyl silane.

Extended Data Figure 2 | Interface formation order.

We adjusted the order of interface formation by casting the water droplet before/after the filling of PDMS as a surrounding media.

Extended Data Figure 3 | Water adhesion-induced droplet distortion.

a, Contact line receding behaviour by pulling the precast water droplet from phenyl silane-modified glass substrate under PDMS−OH (HLB = 0.12) condition. b, Droplet distortion in the pulling condition explains the non-zero adhesion behaviour of the droplet to the substrate.

Extended Data Figure 4 |Water wettability of unmodified glass substrate under PDMS−OH (HLB = 0.12).

Photos of pre/postcast 0.5 μL water droplets under PDMS−OH (HLB = 0.12).

Extended Data Figure 5 |The interfacial energy difference between two configurations.

Simplified scheme and possible interfacial energies of the configuration C and W.

Extended Data Figure 6 |Time dependence on water−PDMS interfacial energy.

Extended Data Figure 7 | Wrapping droplet

Digital microscopic image of a 0.5 μL water droplet wrapped with PDMS−OH (HLB = 0.12). Since the PDMS wrapped droplet has lower interfacial energy (that is, γow + γo =57.9±2.8 mN/m) than bare droplet one (that is, γw =71.6±0.5 mN/m), PDMS−OH spreads to wrap the water droplet. This magnitude relation in interfacial energy is applicable for PDMS (HLB = 0) and PDMS (HLB = 0.73).

Extended Data Figure 8 | HLB effect on the interfacial energy difference of configurations C and W.

Extended Data Figure 9 | Intermolecular interaction between PDMS−NH2 and silanol.

Distance dependence of the intermolecular interaction energy between the −OH groups on the substrate surface and the molecular end group of PDMS−NH2.

Extended Data Figure 10 | PDMS modification effect on pre/postcast water sliding angle.

Sliding angle of 5 μL pre/postcast water droplets under various modified PDMS. The wettability is not branched since both pre/postcast droplets exhibit non-sliding behaviour without dilution by non-modified PDMS.

Extended Data Table 1| Summary of interfacial energies and contact angles of PDMS and water.

| Liquid | Surface tension (in air) [mN/m] | Interfacial tension with water [mN/m] | Static contact angle on probe substrate [°] |
| --- | --- | --- | --- |
| Water | 71.6±0.5 | − | 79.4±1.9 |
| PDMS (HLB = 0) | 19.8±0.3 | 38.1±2.5 | 2.2±0.6 |
| PDMS−OH (HLB = 0.12) | 19.9±0.2 | 20.1±1.7 | 2.0±0.2 |
| PDMS−OH (HLB = 0.73) | 21.4±0.4 | 7.5±0.5 | 14.9±0.6 |
| PDMS−NH2 | 20.5±0.3 | 7.2±0.3 | − |