Supplementary Information for

Controllable tip exposure of ultramicroelectrodes coated by diamond-like carbon via direct microplasma jet for enhanced stability and fidelity in single-cell recording

Zhiyuan Du1,2, Qingda Xu1,2, Ye Xi1,2, Mengfei Xu1,2, Jiawei Cao1,2, Longchun Wang1, Xiuyan Li1, Xiaolin Wang1, Qingkun Liu1, Zude Lin1, Bin Yang1, and Jingquan Liu1*

1 National Key Laboratory of Advanced Micro and Nano Manufacture Technology, Shanghai Jiao Tong University, Shanghai, 200240, China and

2 DCI Joint Team, Collaborative Innovation Center of IFSA, Department of Micro/Nano Electronics, Shanghai Jiao Tong University, Shanghai, 200240, China

*Corresponding author: Jingquan Liu

Email: jqliu@sjtu.edu.cn; Tel: 86-21-34207209; Fax: 86-21-34206883

Table S1

Table S1. Comparison with previous works in recent researchers.

| Author | Exposed tip size | Controllability | Insulation | Encapsulation method |
| --- | --- | --- | --- | --- |
| Pan et al. [28] | Random | - | + | Inserted into wax solution |
| Hunt et al. [29] | 20 μm in length |  |  |  |
| Roberts et al. [14] | 5 μm in length | + | - | Placed into phenolic solution for electro-polymerization |
| Gao et al. [31] | Only a ring on the cross-section | - | ++ | Inserted into wax solution and mechanical polish |
| Xu et al. [15] | Only a ring on the cross-section | - | ++ | Inserted into wax solution and grind by diamond disk |
| Zhang et al. [35] | About 5 μm in length | + | ++ | Inserted into glass micropipette and wax solution |
| Wu et al. [36] | 4 μm in length |  |  |  |
| Jiao et al. [25] | 5 μm in length |  |  |  |
| Jiang et al. [37] | 10 μm in length |  |  |  |
| Xu et al. [38] | 28 μm in length | + | - | Inserted into glass micropipette micromanipulator |
| Xi et al. [44] | 33 μm in length | - | - | Deposited with parylene-C and etched by plasma jet |
| This work | 0.8 μm in length | ++ | ++ | Deposited with DLC and etched by microplasma jet branch |

Technique performance in each work is ranked as follows: –, poor; +, fair; ++, good.

Figure S1

Fig. S1: Biocompatibility testing of the DLC-UME within 7 days.

Equation S1

Eq. S1: Formula for accelerated aging of UMEs.

f =2ΔT/10

Δ T is equal to the difference between the ambient temperature during electrochemical testing and the reference temperature.

Figure S2

Fig. S2: Dynamic potential response of the DLC-UME in solutions with different pH values.