Supplementary Material

Lateral Size-Controlled Single-Layer MoS2 Synthesis via Chemical Vapor Deposition

B.A. Küçük1,2, M.A. Çağlar1,2,3, G. Turgut1,2,3*

12D Material Research Lab., High Technology Research and Application Centre, Erzurum Technical University, 25100 Erzurum, Turkey

2Department of Photonics, Science Institute, Erzurum Technical University, 25100 Erzurum, Turkey

3Department of Basic Sciences, Science Faculty, Erzurum Technical University, 25100 Erzurum, Turkey

The Corresponding author (*):  Güven Turgut

Phone: +90 444 5 333 22 73

e-mail: guven.turgut@erzurum.edu.tr

Adress: Department of Basic Sciences, Science Faculty, Erzurum Technical University, Erzurum, 25100, Turkey

Supplementary Materials :

Figure S1. Diagram of CVD experimental setup during growth of MoS2 flakes

Figure S2. MoS2 growth in alumina boat zones

Figure S3. CVD-grown mechanisims of MoS2 layers for close-ended alumina boat and open-ended quartz boat

Figure S4.MoS2 flakes grown on SiO2/Si substrate , Experimental setup, Photo of experimental

boat,O.M

Table 1. Optimizations of MoS2 grown by CVD have been reported in the literature.

Figure S1. Diagram of CVD experimental setup during growth of MoS2 flakes

Figure S2. MoS2 growth for different zones in alumina boat

Figure S3.  CVD-grown mechanisims of MoS2 layers for close-ended alumina boat and open-ended quartz boat

Figure S4. .MoS2 flakes grown on SiO2/Si substrate , Experimental setup, Photo of experimental boat,O.M

Table 1. Optimizations of MoS2 grown by CVD have been reported in the literature(*DMS; Distance between Mo precursor and substrate, ACVD; Atomopheric Pressure CVD, LCVD; Low Pressure CVD )

| Method | Optimized Parameters | Mo Precursor and Amount | Gas type and flow rate (sccm) | Catalysist Type and Amount | Growth Temperature (°C) | Ramp to growth temperature (°C/min.) | Growth Time (min.) | Growht Substrate Type | Boat Type | Maximum Flake Size (μm) | Ref. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ACVD | Gas flow rate | MoO3 (30 mg) | Ar 15 | NaCl 1mg/ml solution | 670 | / | 15 | SiO2/Si | Quartz | 60 | [1] |
| ACVD | Temperature | MoO2 (10 mg) | Ar 200 | / | 750 | 3 | 15 | SiO2/Si | Alumina | 10-50 | [2] |
| ACVD | DMS | MoO3 (5 mg) | Ar 100 | / | 850 | 8 | 10 | SiO2/Si | / | ~770 nm | [3] |
| ACVD | Gas flow rate | MoO3 (100 mg) | Ar | / | 750 | / | 5 | SiO2/Si | Alumia | / | [4] |
| LCVD | Pressure Temperature Time DMS | MoO3 (1 mg) | Ar 30-1000 | PTAS | 750 | / | 10 | SiO2/Si | Quartz | 150 - mm | [5] |
| ACVD | Temperature | MoO3 (3 mg) | Ar 100 | / | 850 | 18.4 | 5 | SiO2/Si | / | 109 | [6] |
| ACVD | Temperature | MoO3 (10 mg) | Ar 50 | / | 720-780 | 10 | 10 | SiO2/Si | Quartz | 20 | [7] |
| ACVD | Temperature | MoO3 (15 mg)) | Ar 10 | / | 760 | 15 | 30 | SiO2/Si | Quartz | 50 | [8] |
| ACVD | Temperature Time M | MoO3 (2 mg) | Ar 140 | / | 700 | 20 | 15 | SiO2/Si | Quartz | ~10 | [9] |
| LCVD | Temperature DMS | MoO3 (10 mg) | N2 100 | / | 850 | 34 | 20 | Sapphire | / | 90 | [10] |
| ACVD | Temperature | MoO3 (5 mg) | Ar 60 | / | 800 | 10 | 15 | SiO2/Si | Quartz | ~25.3 | [11] |
| LCVD | M/S Temperature | MoO3 (0.9 mg) | N2 10 | PTAS | 620-720 | / | 3 | SiO2/Si | Alumina | 120 | [12] |
| LCVD | DMS | MoO3 (1:13 mg) | Ar 10 | / | 700 | / | 30 | SiO2/Si | Alumina | 80 | [13] |
| ACVD | C.T | MoO3 (36 mg) | Ar+H2 65 (%10) | NACI, BR ve I | 780 | 39 | 20 | SiO2/Si | Quartz | 60 | [14] |
| ACVD | Precursor type Catalysis type Time | MoO3 (6 mg) | Ar 100 | NaNO3 2 mg | 550 | 33 | 12 | SiO2/Si | Alumina | ~10 | [15] |
| ACVD | Precursor type Gas flow rate Time M/S | MoO2 (3 mg) | 10 | / | 760 | 15 | 1 | SiO2/Si | Alumina | 70 | [16] |
| ACVD | Temperature Time Precursor type Gas flow rate | NaOH: SMD:DI 4 :0.5:0.5 | N2 200 | / | 700-800 | / | 18-22 | SiO2/Si | Quartz | 100 | [17] |
| ACVD | M/C.T Gas flow rate G.S Time Temperature Boat type | MoO3 (3 mg) | Ar 15 | NaCI 0.3 | 680 | 10 | 20 | SiO2/Si | Quartz (open-ended) | mm scale /continous film | This Work |

Table 1. Optimizations of MoS2 grown by CVD have been reported in the literature(*DMS; Distance between Mo precursor and substrate, ACVD; Atomopheric Pressure CVD, LCVD; Low Pressure CVD )

References

[1]	L. Zang, L. Chen, D. Tan, X. Cao, N. Sun, C. Jiang, Research on Multi-morphology Evolution of MoS2 in Chemical Vapor Deposition, ChemistrySelect. 6 (2021) 8107–8113. https://doi.org/10.1002/slct.202101843.

[2]	Bilgin, F. Liu, A. Vargas, A. Winchester, M.K.L. Man, M. Upmanyu, K.M. Dani, G. Gupta, S. Talapatra, A.D. Mohite, S. Kar, Chemical Vapor Deposition Synthesized Atomically Thin Molybdenum Disulfide with Optoelectronic-Grade Crystalline Quality, ACS Nano. 9 (2015) 8822–8832. https://doi.org/10.1021/acsnano.5b02019.

[3]	M.H. Johari, M.S. Sirat, M.A. Mohamed, S.N.F. Mohd Nasir, M.A. Mat Teridi, A.R. Mohmad, Effects of Mo vapor concentration on the morphology of vertically standing MoS2 nanoflakes, Nanotechnology. 31 (2020) 0–8. https://doi.org/10.1088/1361-6528/ab8666.

[4]	Y. Cao, X. Luo, S. Han, C. Yuan, Y. Yang, Q. Li, T. Yu, S. Ye, Influences of carrier gas flow rate on the morphologies of MoS2 flakes, Chem. Phys. Lett. 631–632 (2015) 30–33. https://doi.org/10.1016/j.cplett.2015.05.001.

[5]	P. Tummala, A. Lamperti, M. Alia, E. Kozma, L.G. Nobili, A. Molle, Application-oriented growth of a molybdenum disulfide (Mos2) single layer by means of parametrically optimized chemical vapor deposition, Materials (Basel). 13 (2020) 1–13. https://doi.org/10.3390/ma13122786.

[6]	W. Wang, X. Zeng, S. Wu, Y. Zeng, Y. Hu, J. Ding, S. Xu, Effect of Mo concentration on shape and size of monolayer MoS2 crystals by chemical vapor deposition, J. Phys. D. Appl. Phys. 50 (2017) 395501. https://doi.org/10.1088/1361-6463/aa81ae.

[7]	L. Wang, F. Chen, X. Ji, Shape consistency of MoS2 flakes grown using chemical vapor deposition, Appl. Phys. Express. 10 (2017) 2–6. https://doi.org/10.7567/APEX.10.065201.

[8] 	S. Wang, Y. Rong, Y. Fan, M. Pacios, H. Bhaskaran, K. He, J.H. Warner, Shape evolution of monolayer MoS2 crystals grown by chemical vapor deposition, Chem. Mater. 26 (2014) 6371–6379. https://doi.org/10.1021/cm5025662.

[9]	F. Chen, W. Su, The effect of the experimental parameters on the growth of MoS2 flakes, CrystEngComm. 20 (2018) 4823–4830. https://doi.org/10.1039/c8ce00733k.

[10]	Y. Yang, H. Pu, J. Di, S. Zhang, J. Hu, Y. Zang, C. Gao, C. Chen, Influences of temperature gradient and distance on the morphologies of MoS2 domains, AIP Adv. 8 (2018). https://doi.org/10.1063/1.5050652.

[11]	F. Chen, W. Su, S. Zhao, Y. Lv, S. Ding, L. Fu, Morphological evolution of atomically thin MoS2flakes synthesized by a chemical vapor deposition strategy, CrystEngComm. 22 (2020) 4174–4179. https://doi.org/10.1039/d0ce00558d.

[12]	S.Y. Yang, G.W. Shim, S.B. Seo, S.Y. Choi, Effective shape-controlled growth of monolayer MoS2 flakes by powder-based chemical vapor deposition, Nano Res. 10 (2017) 255–262. https://doi.org/10.1007/s12274-016-1284-6.

[13]	S. Smagulova, A. Semenova, E. Zakharkina, P. Vinokurov, Investigation of the properties of two-dimensional molybdenum disulfide films synthesized by the CVD method, IOP Conf. Ser. Mater. Sci. Eng. 693 (2019). https://doi.org/10.1088/1757-899X/693/1/012030.

[14]	W. Wang, H. Shu, J. Wang, Y. Cheng, P. Liang, X. Chen, Defect Passivation and Photoluminescence Enhancement of Monolayer MoS2 Crystals through Sodium Halide-Assisted Chemical Vapor Deposition Growth, ACS Appl. Mater. Interfaces. 12 (2020) 9563–9571. https://doi.org/10.1021/acsami.9b19224.

[15]	S.H. Safeer, M.V.O. Moutinho, A.R.J. Barreto, B.S. Archanjo, O.G. Pandoli, M. Cremona, M.E. Huguenin Maia Da Costa, F.L. Freire, V. Carozo, Sodium-Mediated Low-Temperature Synthesis of Monolayers of Molybdenum Disulfide for Nanoscale Optoelectronic Devices, ACS Appl. Nano Mater. 4 (2021) 4172–4180. https://doi.org/10.1021/acsanm.1c00491.

[16]	T. Chiawchan, H. Ramamoorthy, K. Buapan, R. Somphonsane, Cvd synthesis of intermediate state-free, large-area and continuous mos2 via single-step vapor-phase sulfurization of moo2 precursor, Nanomaterials. 11 (2021). https://doi.org/10.3390/nano11102642.

[17]     S.K. Kang, H.S. Lee, Study on Growth Parameters for Monolayer MoS2 Synthesized by CVD Using Solution-based Metal Precursors, Appl. Sci. Converg. Technol. 28 (2019) 159–163. https://doi.org/10.5757/ASCT.2019.28.5.159.