Synthesis of Ag/Cu decorated 3D self-assembled nanowire TiO2 Photocatalyst for Hydrogen Production: A Promising Pathway towards Sustainable Energy Generation

Sachin Wadhai and Pragati Thakur*

Department of Chemistry, Savitribai Phule Pune University, Ganeshkhind, Pune 411007, India

*Corresponding author email ID : pragati.thakur@unipune.ac.in

Keywords:

Photocatalytic hydrogen production, titania, photocatalysis, morphological study, SPR effect, nanowire

Experimental section, Figure S1 – S9

Experimental section

Synthesis of Pt decorated NWT (Pt-NWT)

The decoration of Pt on NWT was carried out by photo-deposition method. Typically, 200 mg of NWT in 10% 100 mL methanol solution was taken and 0.132 mL of 0.08 M Hexachloroplatinic acid (H2PtCl6) was added as a Pt precursor for the preparation of 1% Pt-NWT. Then this solution was irradiated under UV light for 3h, washed with distilled water and dried at 60o C. Similarly, 0.2, 0.4, 0.5, 0.6 and 0.8 % Pt-NWT (Labelled as 0.2Pt-NWT, 0.4Pt-NWT, 0.5Pt-NWT, 0.6Pt-NWT and 0.8Pt-NWT) were synthesized by varying the amount of Pt precursor in the above synthesis method (Shinde et al. 2018).

Synthesis of Cu decorated NWT (Cu-NWT)

Cu decorated NWT was synthesized by photo-deposition method. For that, typically 0.02 M Copper sulphate solution has been prepared and calculated 1.58 mL of copper sulphate solution mixed with 200 mg of NWT in 10% methanol solution has been carried out for the preparation of 1.0% Cu photocatalyst. The solution has been irradiated in UV light for 3h, washed with distilled water and dried at 60o C. Different Cu % i.e., 0.5, 0.75, 1.0, 1.5 and 2.0 % decorated on NWT, labelled as 0.5Cu-NWT, 0.75Cu-NWT, 1.0Cu-NWT, 1.5Cu-NWT and 2.0Cu-NWT photocatalysts were synthesized by varying the copper sulphate solution.

Fig. S1. (a) Powder XRD pattern recorded on NWT, 0.2Pt-NWT, 0.4Pt-NWT, 0.5Pt-NWT, 0.6Pt-NWT, 0.8Pt-NWT and 1.0Pt-NWT photocatalysts, (b) Powder XRD pattern recorded on NWT 0.5Cu-NWT, 0.75Cu-NWT, 1.0Cu-NWT, 1.5Cu-NWT and 2.0Cu-NWT photocatalysts.

Fig. S2. FTIR spectra of NWT, 0.5Pt-NWT, 1.0Cu-NWT and 0.1Ag/1.0Cu-NWT photocatalysts.

Fig. S3. FESEM micrographs of TiO2 synthesized at different NaOH concentrations (a) at 5M, (b) at 10M, (c) at 15M and (d) at 20M.

Fig. S4. (a-c) FESEM micrograph and (d) EDS report of NWT photocatalyst.

Figure S4d shows EDS spectra of NWT photocatalyst which confirms the presence of 78.82% O and 21.18% Ti atomic percentages. Figure S5d shows the HRTEM image of 0.5Pt-NWT shows the lattice fringes with a d-space value of 0.23 nm corresponding to the (111) plane of Pt and 0.326 nm corresponds to (101) plane of anatase TiO2. Figure S5h shows the HRTEM image of 1.0Cu-NWT shows the lattice fringes with a d-space value of 0.211 nm corresponding to the (111) plane of Cu and 0.326 nm corresponds to (101) plane of anatase TiO2. Results depicted the presence of metal nanoparticles homogeneously dispersed on the NWT surface.

Fig. S5. LR-HRTEM images of (a-d) 0.5Pt-NWT and (e-h) 1.0Cu-NWT photocatalysts.

Fig. S6. BET analysis of P25 TiO2 and NWT (a) nitrogen adsorption-desorption isotherm and (b-c) corresponding BET surface area plot.

Fig. S7. Schematic diagram of NWT showing light harvesting ability by repeated light interaction with NWTs.

Fig. S8. XPS spectra of 0.5Pt-NWT photocatalyst (a) survey scan and high-resolution spectra of (b) Ti 2p, (c) O 1s and (d) Pt 4f.

Fig. S9. Tauc plot graph of the optical band gap energy calculated by extrapolation of the linear part of (αhν)2 versus (hc/λ)

References:

Shinde Y, Wadhai S, Ponkshe A, et al (2018) Decoration of Pt on the metal free RGO-TiO2 composite photocatalyst for the enhanced photocatalytic hydrogen evolution and photocatalytic degradation of pharmaceutical pollutant β blocker. Int J Hydrogen Energy 43:4015–4027. https://doi.org/10.1016/j.ijhydene.2017.10.089