Supplementary Information for

Water structure and local potential distribution at Pt surface in alkaline cation mediated hydrogen evolution regulable by electric field

Contents

Section A. Blank Cyclic Voltammograms of Polycrystalline Pt

Section B. Differential Capacitance Method

Section C. Discussion on the Double Layer Structure

Section D. Additional Results for Interfacial Adsorption Behaviours

Fig. S3-Fig. S12 and Table S1-S6

Section E. HER Reaction Rate Analysis

Section F. Determination of Apparent Activation Energy

Section G. DFT Analysis of Interfacial Dynamics

References

Section A. Blank cyclic voltammograms of polycrystalline Pt

Figure S1. Blank cyclic voltammograms of polycrystalline Pt in alkaline media. (a) LiOH, (b) NaOH, and (c) KOH, with a scan rate of 50 mV s-1. The blue, pink, and yellow regions represent the hydrogen region, the double-layer region, and the oxygen region, respectively.

Section B. Differential Capacitance Method

As is well known, electrodes in contact with an electrolyte solution experience surface tension at the interface, which is linked to the desire to minimize the interfacial area. The stronger the inclination, the higher the surface tension. This phenomenon is also influenced by the polarization potential (φ), making it describable by the electric capillary curve. By deriving the second derivative of the surface tension, we can determine the interfacial differential capacitance (Cd) using the following equation:1-3

Cd=d2γdφ2=dσMdφ                           (S1)

where, γ is the surface tension, σM is the residual charge density at the electrode interface.

As shown in Eq. S1, the differential capacitance Cd changes with the potential φ, indicating that the capacitance of the electrode interface is not a constant. In addition to the method described earlier, the accurate measurement of the differential capacitance can be accomplished through electrochemical impedance techniques. Differential capacitance is crucial in analyzing the model of the double electric layer structure.

Section C. Discussion on the Double Layer Structure

In the Gouy-Chapman-Stern (GCS) model, the potential distribution (φ) within the double-layer is determined by the equilibrium of electrostatic forces between charged species (ions) and dielectric forces. The Poisson-Boltzmann equation, which accounts for electrostatics and ionic concentration effects, serves as a mathematical framework for elucidating this potential distribution. By considering the electrolyte solution conditions and electrode interface characteristics, the GCS model enables the prediction and analysis of the potential distribution in the double layer. This understanding is crucial for interpreting diverse electrochemical phenomena and processes.

In this study, experiments were carried out in a 0.1 M MOH (Li+, Na+, K+) solution, representing a symmetric electrolyte where cations and anions carry equal charges. As a result, the potential gradient in the double layer can be modeled using the Poisson-Boltzmann equation:

dφdx=-(8kTNAC*εr)1/2sinh(zeφ2kT)                 (S2)

where, k represents the Boltzmann constant, T denotes the temperature, NA stands for Avogadro's constant, εr indicates the relative dielectric constant of the solution (taken as 6.95×10−10  F m-1 for dilute solutions), C∗ represents the concentration of the solution, z signifies the charge number of the ion, e represents the elementary charge, and φ denotes the potential.

For the diffusion layer (x≥x2):

φ2φdφsinh (zeφ/2kT)=-(8kTNAC*εr)1/2x2xdx               (S3)

By integration, we get:

tanh(zeφ/4kT)tanh(zeφ2/4kT)=e-κ(x-x2)                       (S4)

here: φ2 is the potential corresponding to the outer Helmholtz layer x2, and κ=(2NAC*z2e2εrkT)1/2.

The electric potential drops in the double layer is:

φ0=φ2-(dφdx)x=x2x2                      (S5)

here: φ0 is the potential corresponding to the electrode interface (x = 0).

In the double-layer, the charge density between the electrode interface and OHP (0<x<x2) is zero, and the charge exists in the dispersion layer (x≥x2). According to Gauss's law:

σM=-σS=-εrdφdxx=x2=(8kTNAC*εr)1/2sinh(zeφ2/2kT)      (S6)

here, σM represents the charge density on the metal side, and σS is the charge density in the diffuse layer.

Therefore, the differential capacitance is given by:

1Cd=dφ0dσM=x2εr+1(2εrz2e2NAC*/kT)1/2cosh(zeφ2/2kT)            (S7)

This equation reveals that the relationship between x2 and its corresponding potential φ2 can be established based on the differential capacitance value. However, it does not allow for the independent determination of the specific values of x2 and φ2. Nevertheless, it is evident that the right-hand side (RHS) of this equation consists of two independent terms, corresponding to the capacitance CH of the charges on OHP (0<x<x2) and the capacitance CD of the charges in the diffuse layer (x2<x). Therefore, although the real values of x2 and φ2 cannot be simultaneously obtained through this equation, they can be determined by making reasonable assumptions.

Determination of OHP Center x2:

Under the assumption that the diffusion layer's far end infinitely approaches the centre of OHP, implying that the diffusion layer's thickness tends to be zero and charges are concentrated on the OHP, the capacitance CD equals zero for the charges in the diffusion layer. In this context, it is reasonable to consider that the total capacitance is solely contributed by the capacitance CH of the charges on OHP. Therefore:

1Cd=dφ0dσM=x'2εr                          (S8)

namely

x'2=εrCd                             (S9)

Determination of potential φ2 corresponding to OHP center x2:

For the potential φ2 at the OHP centre x2, assuming that the solvated cations infinitely approach the electrode surface, i.e. x2 tends to be zero, the capacitance CH from the charges on the OHP becomes negligible. In this scenario, the total capacitance primarily determined by the capacitance CD of the charges in the diffuse layer. Thus:

Cd=(2εrz2e2NAC*/kT)1/2cosh(zeφ'2/2kT)         (S10)

In addition to the methods mentioned above, x2 can also be determined through DFT calculation. By using the predicted results and incorporating them into Eq. S6, the value of φ2 can be calculated, thereby enabling the determination of the potential drop Ψ0 across the entire double layer. It is evident that the GCS model analyzes the diffuse layer by assuming that the electric potential at the end of the diffuse layer φS = 0. Consequently, in numerical terms, the electric potential of the double layer Ψ0 = φ0 and the electric potential of the diffuse layer Ψ1 = φ2.

Double layer structure under the action of directional external electric field:

When an external electric field is introduced, it has a substantial impact on the ion distribution in the solution. In such scenarios, adjustments to the GCS model become essential. When a uniform electric field is applied in the opposite direction to the internal electric field throughout the system, the potential gradient is expressed as:

dφdx-Vm=-(8kTNAμC*εr)1/2sinh(zeφ2kT)                (S11)

where, φ is the potential without the external electric field, V is the voltage of the uniform electric field, m is the distance between the two electrodes, and μ is a constant. For Eq. S11, the electric field strength at x2 is:

(dφdx)x=x2=-8kTNAμC*εr12sinh(zeφ22kT)+Vm               (S12)

The electric potential drops in the double-layer is:

φ0*=φ2*-(dφdx)x=x2*x2*                  (S13)

where, φ0* represents the corrected potential at x=0, x2* denotes the corrected center of the OHP, and φ2* represents its corresponding potential.

The differential capacitance after applying an external electric field is:

1Cd*=dφ0*dσM=x2*εr+1(2εrz2e2NAC*/kT)1/2cosh(zeφ2*/2kT)           (S14)

Figure S2. (a) Schematic diagram of the classical metal-solid/liquid interface double layer structure, in which purple circles represent metal cations and white circles are water molecules. The inner Helmholtz layer (IHP) center (x1), the outer Helmholtz layer (OHP) center (x2), the metal surface potential (φ0), the potential at IHP (φ1), the potential at OHP (φ2), the potential drop of the entire double electric layer (Ψ0), the dispersion layer potential drop (Ψ1), and the metal surface charge density (σM) are labeled on proper position. (b) Double-layer potential (φ) distribution in alkaline media obtained by Gouy-Chapman-Stern model.

For AM+ with a volume concentration of 0.1 M, each AM+ occupies an average volume of 16.7 nm3, approximated as a cube with a side length of 2.55 nm, resulting in a surface density of 1.54 × 1013 cm-2. Following the double-layer capacitor approximation, the charged amount on a single electrode surface is calculated as Q=CΨ0. Utilizing potentials of 124.0 mV, 109.9 mV, and 99.8 mV, the surface densities are determined as 13.28 × 1013 cm-2, 9.64 × 1013 cm-2, and 7.63 × 1013 cm-2 for K+, Na+ and Li+, respectively. These values notably exceed the bulk concentrations (8.6, 6.3, and 5.0 times the bulk concentration), indicating substantial local accumulation at the electrode surface. The local accumulation rate of K+ surpasses that of Li+ and Na+ by 72% and 36%, respectively. This data indicates the significant local accumulation of ions at the electrode surface under the given conditions, with K+ showing the highest accumulation rate among the three ions.

Section D. Additional Results for Interfacial Adsorption Behaviours

Figure S3. Differential capacitance curves obtained by employing the scanning potential method in solutions of H2SO4 (a), H2SO4+KCl (b), KCl (c), KCl+KOH (d), and KOH (e).

In Fig. S3, the pH increases from (a) to (e), resulting in a significant difference in capacitance characteristics between acidic and alkaline solutions. Capacitance values can be converted into surface ion adsorption density, which is notably higher than densities calculated from electrolyte concentration. For instance, using KOH at a 0.1 M concentration yields a 28-fold difference in ion surface density between the two methods. The higher local effective concentrations of cations at the electrode surface suggest that surface-adsorbed alkali metal cations play a crucial role in influencing surface HER kinetics, aligning with previous research findings.4,5 Possible explanations for the discrepancies include aggregation effects and considerations of layer thickness in the differential capacitance method. However, the explanation of aggregation effects fails when interpreting results in 0.05 M H2SO4 where capacitance reaches the mF level shown in Fig. S3(a) requiring unreasonably high ion surface density. Therefore, we cannot treat the electrical double layer (EDL) as atomic thin layer. For KOH, a thickness of 66.3 nm for EDL is estimated.

A notable finding is the stronger adsorption of H ions in alkaline solution compared to neutral one, as depicted in Figs. S3(c) and (e). Even in alkaline solutions, there is observable H+ ion adsorption, suggesting the presence of H3+O in highly alkaline environments, in line with prior reports.6 The introduction of OH- enhances H adsorption indicates that OH- is more effective in facilitating H adsorption on Pt surface than Cl-. In Fig. S3, two distinct H adsorption peaks are evident, indicating the presence of different valence states on Pt surface, Pt0 and Ptn+, consistent with earlier reports on Ru metal.7 It is evident that HBE does not exhibit a positive correlation with HER activity, necessitating consideration of other factors, aligning with previous literature conclusions.8

Under alkaline conditions, the presence of hydroxide groups (OH-) leads to a strong binding of AM+ to the negatively charged electrode surface through electrostatic interactions within the double layer region. Within IHP, active sites are strongly bound to structural water (SW), while in OHP, AM+ is densely adsorbed on the electrode surface based on its hydration ability. Additionally, they promote catalysts by activating the O-H bonds of water through p-orbital interaction between the O atom and SW of water reactants, facilitating the cleavage of O-H by reducing the reaction barrier of water dissociation.9

Due to their limited hydration capacity, the large K+ cations are weakly hydrated and adsorbed with more free water at the electrode surface, hindering the diffusion of water to the active sites and consequently diminishing the HER activity. In reality, solely considering the electrostatic interaction, the electrode surface should exhibit denser coverage upon the introduction of Li+, which possesses the strongest structure-blocking tendency. This is due to the formation of a local “water-in-salt” structure at the nanoscale interface,10 potentially resulting in the lowest chemical reactivity as it blocks the active sites.

Figure S4. Blank cyclic voltammogram of Pt in 0.05 M H2SO4 solution. Scan rate: 50 mV s-1.

Table 1. AM+ double layer characteristic data of Pt in 0.1M alkaline medium

| AM+ | Adsorption potential/V | Cd /μF cm-2 | σM /μC cm-2 | x′2 /Å | φ′2 /mV | φ0 /mV | Ψ0 /mV | Ψ1 /mV |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Li+ | 0.41 | 122.36 | 5.06 | 5.68 | 57.4 | 99.8 | 99.8 | 57.4 |
| Na+ | 0.43 | 140.36 | 6.18 | 4.95 | 65.9 | 109.9 | 109.9 | 65.9 |
| K+ | 0.44 | 171.42 | 7.98 | 4.05 | 77.5 | 124.0 | 124.0 | 77.5 |

Figure S5. Voltammetry curves of polycrystalline Pt electrode in alkaline medium (pH=13, NaOH, KOH) under DEEF. LSV curves with a scanning rate of 5 mV s-1 in NaOH (a) and KOH (c) solutions with iR compensation. CV curves with a scanning rate of 50 mV s-1 in LiOH (b) and KOH (d) solutions.

Figure S6. Chronoamperometric method to determine the effect of DEEF on HER rate of Pt in alkaline medium, pH=13, LiOH (a), NaOH (b), KOH (c). The results are consistent with those from LSV tests. Significant effects on the HER catalytic rate are observed by controlling the cations through the applied DEEF. The red traces represent the current response without the applied DEEF, while the blue traces represent the current response with the applied DEEF. The testing potential is -0.088 V vs. RHE.

Figure S7. Voltammetry curves of polycrystalline Pt electrode in alkaline medium (pH=13, NaOH, KOH) under the difference DEEF intensity, with 0 V (a), 5 V (b), 25 V (c).

Table S2. Overpotentials of Pt at 10 mA cm-2 in alkaline medium under DEEF

|  | LiOH | NaOH | KOH |
| --- | --- | --- | --- |
| 5V | 88 | 87 | 87 |
| 10V | 85 | 79 | 72 |
| 15V | 82 | 73 | 70 |
| 20V | 80 | 70 | 69 |
| 25V | 77 | 68 | 67 |

Figure S8. (a) Blank cyclic voltammogram of Pt in LiOH solution under the influence of DEEF. The black dashed box in (a) represents the hydrogen underpotential deposition peak. (b) Zoom-in view of the black boxed region in (a). Integration of the hydrogen underpotential deposition peak is performed to estimate the amount of hydrogen adsorbed at the electrode interface.

Table S3. Relationship between DEEF intensity and integrated area of hydrogen underpotential deposition peaks

| DEEF voltage (V) | Hydrogen adsorption capacity (LiOH) |
| --- | --- |
| 0 | 115.59 |
| 5 | 104.41 |
| 10 | 97.08 |
| 15 | 91.99 |
| 20 | 90.85 |
| 25 | 89.01 |

Figure S9. Voltametric characteristics of polycrystalline Pt electrode in H2SO4 solution under the influence of DEEF. The scan rate is 5 mV s-1 with iR compensation.

Figure S10. Schematic diagram of dynamic differential capacitance curve measurement. Here, CE, RE and WE denote the counter electrode, reference electrode, and the working electrode, respectively.

Figure S11. Electrochemical study of Pt electrode in alkaline medium (NaOH, KOH) under DEEF. DDC results of Pt electrode in NaOH (a) and KOH (d). The dependence of HER catalytic activity of Pt (overpotential at 10 mA cm-2) on the adsorption capacitance of Na+ (b) and K+ (e). The relationship between the electric potential distribution of double-layers and the DEEF intensity in NaOH (c) and KOH (f) solutions.

Table S4. AM+ double-layer characteristic data of Pt under DEEF in 0.1 M of different alkaline medium

| AM+ | Adsorption potential/V | DEEF voltage/V | C*d /μF cm-2 | σM /μC cm-2 |  | x*2 /Å | φ*2 /mV | φ*0 /mV | Ψ*0 /mV | Ψ*1 /mV |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Li+ | 0.41 | 0 | 137.68 |  | 6.02 | 5.05 | 64.8 | 108.5 | 108.5 | 64.8 |
|  |  | 5 | 133.64 |  | 5.77 | 5.20 | 63.0 | 106.2 | 106.2 | 63.0 |
|  |  | 10 | 121.38 |  | 5.01 | 5.72 | 57.0 | 98.2 | 98.2 | 57.0 |
|  |  | 15 | 119.69 |  | 4.90 | 5.80 | 56.1 | 97.0 | 97.0 | 56.1 |
|  |  | 20 | 119.18 |  | 4.87 | 5.83 | 55.8 | 96.7 | 96.7 | 55.8 |
|  |  | 25 | 117.98 |  | 4.79 | 5.89 | 55.2 | 95.8 | 95.8 | 55.2 |
| Na+ | 0.43 | 0 | 146.27 |  | 6.53 | 4.75 | 68.4 | 113.0 | 113.0 | 68.4 |
|  |  | 5 | 137.04 |  | 5.98 | 5.07 | 64.5 | 108.1 | 108.1 | 64.5 |
|  |  | 10 | 135.41 |  | 5.88 | 5.13 | 63.8 | 107.2 | 107.2 | 63.8 |
|  |  | 15 | 132.34 |  | 5.69 | 5.25 | 62.4 | 105.4 | 105.4 | 62.4 |
|  |  | 20 | 130.98 |  | 5.61 | 5.30 | 61.7 | 104.5 | 104.5 | 61.7 |
|  |  | 25 | 127.34 |  | 5.39 | 5.46 | 60.0 | 102.3 | 102.3 | 60.0 |
| K+ | 0.44 | 0 | 146.56 |  | 6.55 | 4.74 | 68.5 | 113.2 | 113.2 | 68.5 |
|  |  | 5 | 146.42 |  | 6.54 | 4.75 | 68.4 | 113.1 | 113.1 | 68.4 |
|  |  | 10 | 144.13 |  | 6.40 | 4.82 | 67.5 | 111.9 | 111.9 | 67.5 |
|  |  | 15 | 143.07 |  | 6.34 | 4.86 | 67.1 | 111.4 | 111.4 | 67.1 |
|  |  | 20 | 130.85 |  | 5.60 | 5.31 | 61.7 | 104.5 | 104.5 | 61.7 |
|  |  | 25 | 110.65 |  | 4.31 | 6.28 | 50.9 | 89.8 | 89.8 | 50.9 |

Table S5. AM+ density retention rate (%) in EDL under DEEF in 0.1 M alkaline medium

| DEEF voltage/V | LiOH | NaOH | KOH |
| --- | --- | --- | --- |
| 0 | 100.00 | 100.00 | 100.00 |
| 5 | 95.01 | 89.63 | 99.82 |
| 10 | 79.79 | 87.82 | 97.21 |
| 15 | 77.72 | 84.39 | 96.07 |
| 20 | 77.15 | 82.81 | 82.42 |
| 25 | 75.66 | 78.81 | 59.89 |

Table S6. OH- adsorption data of Pt under DEEF in 0.1 M of different alkaline medium

| DEEF voltage/V | LiOH | NaOH | KOH |
| --- | --- | --- | --- |
| 5 | 138.33 | 139.63 | 145.91 |
| 10 | 125.08 | 136.27 | 144.44 |
| 15 | 124.08 | 134.75 | 142.91 |
| 20 | 123.55 | 132.33 | 133.36 |
| 25 | 122.35 | 126.78 | 112.02 |

Figure S12. Tafel slopes of Pt in 0.1 M NaOH (a) and KOH (b) solutions under the influence of DEEF.

Section E. HER Reaction Rate Analysis

The influence factors of Tafel slope exceeding 120 mV dec-1 in Volmer rate-determinate step in HER process were analyzed. The influence of electrode surf ace hydrogen coverage θH on reaction rate in Heyrovsky rate-limiting step was also analyzed.11,12

When the Volmer step is the rate-determining step:

H2O + e- + * = H* + OH-                (S15)

the forward reaction rate is the total rate:

j=nFkf0aH2Oexp(-αFRTη)                 (S16)

where, j is the current density (mA cm-2), n=1, F=96485 C mol-1, aH2O=1, R=8.314 J K-1 mol-1, T=298.15 K, η stands for overpotential. Using kf0 and α as unknown variables, we can explore the response of Log(j) to η. When α<0.5, the resulting Tafel slope value is more than 120 mV dec-1, as shown in Fig. S12 and Table S4.

Figure S13. Microdynamic modeling of the Volmer rate-determining step in HER. Calculations demonstrate that the Tafel slope is limited by the Volmer step, with kf0 varying by 10 orders of magnitude, while α varying between 0.3 and 0.5. The results show that α is more sensitive to changes in the Tafel slope than kf0.

Table S7. Microdynamic modeling of the Volmer rate-determining step in HER

| kf。 (s-1) | Calculated Tafel slope (mV dec-1) at η = -0.50 V for α = 0.3 | Calculated Tafel slope (mV dec-1) at η = -0.50 V for α = 0.4 | Calculated Tafel slope (mV dec-1) at η = -0.50 V for α = 0.5 |
| --- | --- | --- | --- |
| 10-5 s-1 | 197 | 148 | 118 |
| 1 s-1 | 197 | 148 | 118 |
| 105 s-1 | 197 | 148 | 118 |

When the Heyrovsky step is the rate-determining step,

H2O + e- + H* = H2 + OH- + *             (S17)

the forward reaction rate corresponds to the total reaction rate, which depends on the surface hydrogen coverage θH:

j = nFk2 0aH2O exp (-αFRTη) θH              (S18)

θH=KVolmeraH2OaOH-exp(fη)+KVolmeraH2O                (S19)

where, k2 0=10-5 s-1, α=0.5, f=F/RT, KVolmer is the reaction equilibrium constant for the Volmer step and is taken as 0.05. Based on this, we can investigate the effect of OH- ion activity (aOH-) on the hydrogen coverage (θH), and thereby understand its influence on the response of Log(j) and η. The aOH- is related to its concentration C as follows: aOH-= λCOH-, where λ is the activity coefficient. For dilute solutions, the activity coefficient λ tends to be 1, and the ion activity is approximately equal to its ion concentration. Additionally, as discussed earlier, under the influence of DEEF, the OH- concentration within EDL at electrode interface decreases with increasing DEEF strength. Therefore, we will discuss the influence of aOH- within the range of 0.02 to 0.1 on the hydrogen coverage θH, as shown in Fig. S13.

Figure S14. Microdynamic modeling of Heyrovsky rate-determining step in HER. Hydrogen surface coverage θH and Tafel slope are calculated from the HER microkinetic model subject to the Heyrovsky step limit. The results show that the θH increases with decreasing OH- concentration at the same overpotential. The change in the calculated Tafel slope as a function of overpotential is captured by the increase in θH. A shift in Tafel slope from low to high overpotential occurred at approximately θH ≈ 0.6, consistent with previous reports.11 At the same time, as the concentration of OH- decreases, this shift occurs at lower overpotential.

Section F. Determination of Apparent Activation Energy

The determination of apparent activation energy involves fitting the Butler-Volmer equation to the linear sweep voltammetry curves obtained at various temperatures using the least squares method, resulting in the determination of the exchange current density j0 (mA cm-²) and the charge transfer coefficient α. The Butler-Volmer equation is as follows:

j=j0[eαFRTη-e[-(1-α)FRT]η]                (S20)

Where, j represents current density (mA cm-²), F=96485 C mol-1, R=8.314 J K−1 mol−1, T is the experimental temperature, and η denotes overpotential (V). Subsequently, the apparent activation energy, EA,app (kJ/mol), is determined using the modified Arrhenius equation. The logarithmically transformed Arrhenius equation is as follows:

ln⁡(j0)=lnA-EA,appR(1T)                (S21)

where, A represents the pre-exponential factor.

To ensure that the result does not depend on the analytical method but on the properties of the Pt electrode itself, the apparent activation energy obtained based on the Tafel extrapolation is compared with the apparent activation energy from fitting the Butler-Volmer equation. Extrapolation from the linear region in the Tafel plot yields the intercept ln(j0) at the overpotential η = 0, which in turn leads to the exchange current density j0. The above equation is then applied to calculate the apparent activation energies.

Figure S15. Temperature-dependent HER measurements of polycrystalline Pt in alkaline media NaOH (a) and KOH (b). The temperature range for the test is 30 °C to 50 °C with intervals of 5°C. The red dashed lines represent the fitting curves by Butler-Volmer equation.

Figure S16. Exploring the apparent activation energies of Pt in KOH solution with DEEF. The applied external E-field voltages are 5 V (a), 10 V (b), 15 V (c), and 20 V (d).

Figure S17. Comparison of apparent activation energies extracted with the Butler-Volmer equation fitting method and the Tafel extrapolation method. For Pt electrodes, the results calculated by both methods are similar, where blue color represents the Tafel extrapolation method and red color represents the Butler-Volmer fitting method.

Section G. DFT Analysis of Interfacial Dynamics

Figure S18. Pure water system. (a) Side view of Pt (111)/water interface model. Red, pink and gray spheres represent O, H, and Pt atoms, respectively. (b) Schematic diagram of the angle (θ) between the water molecule bisector and the normal of the Pt surface. (c) Two-dimensional probability distribution of θ as a function of the height (h) above the electrode surface.

Figure S19. Two-dimensional probability distribution of θ as a function of h in the (a) Li+, (b) Na+, and (c) K+ systems.

Figure S20. Representative snapshots of the Pt(111)/water interface in (a) Li+, (b) Na+, (c) K+, and (d) pure water systems. The water molecules within the blue circles are those directly covalently interacting with Pt in the pure water system, which, upon the introduction of cations, are influenced by the cations and transited to covalent or non-covalent interactions with the cations.

Table S8. Summary of DFT calculation characteristic data in Li+, Na+, K+, and pure water systems

| Systems | Coordination number (CN) | Pt-AM+ distance | AM+-O bond length | Average distance between water and Pt surface | θ |
| --- | --- | --- | --- | --- | --- |
| Li+ | 4 | 5.22 Å | 2.01 Å | 4.22 Å | 118.24 º |
| Na+ | 4 | 4.43 Å | 2.30 Å | 4.26 Å | 117.34 º |
| K+ | 5 | 3.01 Å | 2.87 Å | 4.54 Å | 95.29 º |
| Pure H2O | / | / | / | 4.14 Å | 92.98 º |

References

1.	Wu, J. Z. Understanding the Electric Double-Layer Structure, Capacitance, and Charging Dynamics. Chem. Rev. 122, 10821-10859, (2022).

2.	Zhan, C., Lian, C., Zhang, Y., Thompson, M. W., Xie, Y., Wu, J. Z., Kent, P. R. C., Cummings, P. T., Jiang, D. E. & Wesolowski, D. J. Computational Insights into Materials and Interfaces for Capacitive Energy Storage. Adv. Sci. 4, 1700059, (2017).

3.	Garcia-Araez, N., Climent, V., Herrero, E., Feliu, J. M. & Lipkowski, J. Thermodynamic approach to the double layer capacity of a Pt(111) electrode in perchloric acid solutions. Electrochim. Acta 51, 3787-3793, (2006).

4.	Xue, S., Garlyyev, B., Auer, A., Kunze-Liebhäuser, J. & Bandarenka, A. S. How the Nature of the Alkali Metal Cations Influences the Double-Layer Capacitance of Cu, Au, and Pt Single-Crystal Electrodes. J. Phys. Chem. C 124, 12442-12447, (2020).

5.	Garlyyev, B., Xue, S., Watzele, S., Scieszka, D. & Bandarenka, A. S. Influence of the Nature of the Alkali Metal Cations on the Electrical Double-Layer Capacitance of Model Pt(111) and Au(111) Electrodes. J. Phys. Chem. Lett. 9, 1927-1930, (2018).

6.	Wang, X., Xu, C., Jaroniec, M., Zheng, Y. & Qiao, S.-Z. Anomalous hydrogen evolution behavior in high-pH environment induced by locally generated hydronium ions. Nat. Commun. 10, 4876, (2019).

7.	Palaniappan, R. & Botte, G. G. Effect of Ammonia on Pt, Ru, Rh, and Ni Cathodes During the Alkaline Hydrogen Evolution Reaction. Journal of Physical Chemistry C 117, 17429-17441, (2013).

8.	Monteiro, M. C. O., Goyal, A., Moerland, P. & Koper, M. T. M. Understanding Cation Trends for Hydrogen Evolution on Platinum and Gold Electrodes in Alkaline Media. ACS Catal. 11, 14328-14335, (2021).

9.	Wang, P.-Y., Zhou, J.-F., Chen, H., Peng, B. & Zhang, K. Activation of H2O Tailored by Interfacial Electronic States at a Nanoscale Interface for Enhanced Electrocatalytic Hydrogen Evolution. JACS Au 2, 1457-1471, (2022).

10.	Suo, L., Borodin, O., Gao, T., Olguin, M., Ho, J., Fan, X., Luo, C., Wang, C. & Xu, K. “Water-in-salt” electrolyte enables high-voltage aqueous lithium-ion chemistries. Science 350, 938-943, (2015).

11.	Shinagawa, T., Garcia-Esparza, A. T. & Takanabe, K. Insight on Tafel slopes from a microkinetic analysis of aqueous electrocatalysis for energy conversion. Sci. Rep. 5, 13801, (2015).

12.	Tang, M. T., Liu, X. Y., Ji, Y. F., Norskov, J. K. & Chan, K. R. Modeling Hydrogen Evolution Reaction Kinetics through Explicit Water-Metal Interfaces. J. Phys. Chem. C 124, 28083-28092, (2020).