| Table 1: Factor levels of the BBD design for MV2B removal by CS/Alg/FA |  |  |  |  |
| --- | --- | --- | --- | --- |
| Factor name | Factor code | Level of factor |  |  |
|  |  | -1 | 0 | 1 |
| CS/Alg/FA Dose (g/100mL) | A | 0.02 | 0.06 | 0.1 |
| Solution pH | B | 4 | 7 | 10 |
| Time (min) | C | 20 | 100 | 180 |

Table 2: The 3-variables BBD matrix and experimental data for MV2B removal (%) by CS/Alg/FA Run; A: CS/Alg/FA dose (g); B:pH; C:Time (min); MV2B removal (%). 1; 0.02; 4; 100; 15.5. 2; 0.1; 4; 100; 65.1. 3; 0.02; 10; 100; 58.4. 4; 0.1; 10; 100; 78.4. 5; 0.02; 7; 20; 4.8. 6; 0.1; 7; 20; 63.5. 7; 0.02; 7; 180; 50.3. 8; 0.1; 7; 180; 65.2. 9; 0.06; 4; 20; 5.7. 10; 0.06; 10; 20; 30.7. 11; 0.06; 4; 180; 17.9. 12; 0.06; 10; 180; 59.9. 13; 0.06; 7; 100; 63.4. 14; 0.06; 7; 100; 60.5. 15; 0.06; 7; 100; 65.8. 16; 0.06; 7; 100; 66.4. 17; 0.06; 7; 100; 63.6.

| Table 3: BET analysis of CS/Alg/FA |  |
| --- | --- |
| Parameters | CS/Alg/FA |
| Surface Area (m2/g) | 1.43 |
| Langmuir Surface Area (m2/g) | 16.5 |
| Total Volume in Pore (cm3/g) | 0.0023 |
| Average Pore Diameter (nm) | 14.4 |

| Table 4: ANOVA test results for MV2B removal by CS/Alg/FA |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Source | Sum of Squares | df | Mean Square | F-value | p-value | Significant |
| Model | 9155.94 | 9 | 1017.33 | 165.47 | < 0.0001 | * |
| A-Dose | 2563.28 | 1 | 2563.28 | 416.92 | < 0.0001 | * |
| B-pH | 1897.28 | 1 | 1897.28 | 308.59 | < 0.0001 | * |
| C-Time | 981.24 | 1 | 981.24 | 159.60 | < 0.0001 | * |
| AB | 219.04 | 1 | 219.04 | 35.63 | 0.0006 | * |
| AC | 479.61 | 1 | 479.61 | 78.01 | < 0.0001 | * |
| BC | 72.25 | 1 | 72.25 | 11.75 | 0.0110 | * |
| A² | 63.88 | 1 | 63.88 | 10.39 | 0.0146 | * |
| B² | 767.94 | 1 | 767.94 | 124.91 | < 0.0001 | * |
| C² | 2020.33 | 1 | 2020.33 | 328.61 | < 0.0001 | * |
| Residual | 43.04 | 7 | 6.15 |  |  |  |
| Lack of Fit | 20.79 | 3 | 6.93 | 1.25 | 0.4041 | # |
| Pure Error | 22.25 | 4 | 5.56 |  |  |  |
| Cor total | 9198.98 | 16 |  |  |  |  |
| R2 | 0.9953 |  |  |  |  |  |
| Adjusted R2 | 0.9893 |  |  |  |  |  |

* Significant; # not significant.

Table 5: Adsorption kinetics & isotherms nonlinear models and adsorption thermodynamic. Models; Equations; Parameters. Pseudo-first order (PFO); qt=qe1-e-k1t; k1: pseudo-first-order rate constant (1/min). Pseudo-second order (PSO); qt=qe2k2t1+ qek2t; k2: pseudo-second-order rate constant (g/mg min). Langmuir; qe=qmKLCe1+ KLCe; qm: monolayer capacity (mg/g) KL : Langmuir constant (L/mg). Freundlich; qe=KFCe1n; KF: Freundlich constant (mg/g) (L/mg)1/n n: adsorption intensity. Temkin; qe=RTbTlnKTCe; KT: Temkin constant (L/mg) : heat of adsorption(J/mol). Adsorption thermodynamic; ∆Go=RTlnkd; ΔG°: Gibbs free energy change. ln kd=∆SoR-∆HoRT; ΔS°: Entropy change ΔH°: Enthalpy change. kd=qece; kd : Partition coefficient.

| Table 6: Kinetic model data for MV2B adsorption by CS/Alg/FA (CS/Alg/FA dose=0.1g/100mL; pH=10; temperature=25°C; agitation speed=80strokes/min) |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Concentration (mg/L) | qe exp. (mg/g) | PFO |  |  |  | PSO |  |  |
|  |  | qe cal (mg/g) | k1 (1/min) | R2 |  | qe cal (mg/g) | k2 x 10-2 (g/mg.min) | R2 |
| 20 | 14.5 | 14.5 | 3.54 | 1.00 |  | 14.7 | 0.58 | 0.94 |
| 50 | 25.6 | 25.8 | 0.77 | 0.99 |  | 25.9 | 0.33 | 0.99 |
| 80 | 39.3 | 40.6 | 0.51 | 0.99 |  | 41.1 | 0.06 | 0.99 |
| 120 | 44.4 | 47.7 | 0.62 | 0.99 |  | 47.8 | 0.11 | 0.99 |
| 150 | 52.8 | 54.2 | 0.87 | 0.99 |  | 54.3 | 0.27 | 0.99 |
| 200 | 56.1 | 48.9 | 0.09 | 0.93 |  | 54.1 | 0.002 | 0.97 |
| 250 | 61.4 | 56.9 | 0.05 | 0.95 |  | 64.1 | 0.001 | 0.98 |

| Table 7: Isotherm model parameters for MV2B removal by CS/Alg/FA |  |  |
| --- | --- | --- |
| Adsorption isotherm | Parameter | Value |
| Langmuir | qmax (mg/g) | 63.4 |
|  | Ka (L/mg) | 0.12 |
|  | R2 | 0.94 |
| Freundlich | Kf (mg/g) (L/mg)1/n | 23.7 |
|  | n | 5.06 |
|  | R2 | 0.88 |
| Temkin | KT (L/mg) | 4.31 |
|  | bT (J/mol) | 257.9 |
|  | R2 | 0.94 |

| Table 8: Comparison of adsorption capacity of CS-BD/Alg/FA for MV2B removal with other adsorbents |  |  |
| --- | --- | --- |
| Adsorbents employed for MV dye removal | Maximum adsorption capacity (mg/g) | Reference |
| CS/Alg/FA | 63.4 | Present study |
| # Coal-based activated carbon | 134.1 | [61] |
| Clay/starch/Fe3O4 nanocomposite | 29.67 | [62] |
| Montmorillonite clay/starch/CoFe2O4 nanocomposite | 47.51 | [63] |
| Zeolite Clay/Fe-Al Hydrotalcite composite | 81.98 | [64] |
| Algae modified Schiff base-chitosan benzaldehyde composite | 126.51 | [65] |
| Magnetite carboxymethylcellulose | 107.78 | [66] |
| Glutaraldehyde cross-linked alginate/sepiolite hydrogel capsules | 357.1 | [67] |
| porous material polyacrylamide/ astragalus membranaceus/attapulgite | 709.13 | [68] |
| Magnetic chitosan microspheres | 128.84 | [69] |

| Table 9 : Thermodynamic parameters of MV2B removal by Cs-Alg-FA |  |  |  |  |
| --- | --- | --- | --- | --- |
| Temperature (K) | lnkd | ∆G (kJ/mol) | ∆H (kJ/mol) | ∆S (J/mol.K) |
| 298.15 | 0.54 | -1.26 | 42.6 | 0.15 |
| 308.15 | 1.07 | -2.73 |  |  |
| 318.15 | 1.48 | -4.21 |  |  |
| 328.15 | 2.16 | -5.68 |  |  |