Supplementary Information

Operando Neutron Imaging-guided Gradient Design of Li-ion Solid Conductor for Extremely High Mass-loading Cathodes

Tongtai Ji1, Yuxuan Zhang2, James Torres2, Jean-Christophe Bilheux2, Jiwei Wang1, Hongli Zhu1, *

1Department of Mechanical and Industrial Engineering, Northeastern University, 360 Huntington Avenue, Boston, Massachusetts 02115, United States

2Neutron Scattering Division, Oak Ridge National Laboratory, Oak Ridge, Tennessee 37831, USA.

*: Corresponding author: h.zhu@neu.edu

(Front view)

(Side view)

Supplementary Figure 1. Pictures of the setup of the Operando neutron imaging on Multimodal Advanced Radiography Station (MARS), HFIR beamline CG-1D, at Oak Ridge National Laboratory

Supplementary Figure 2. Charge and discharge profile for the Operando neutron imaging cell with thick cathode (33.3mg/cm2), and the Operando electrochemical impedance spectroscopies (EISs) collected during cycling.

Supplementary Figure 3. Schematic of the sampling area for the neutron imaging analysis

Supplementary Figure 4. Zoomed-in neutron transmission change (Trt/Tr0) for the thick cathode layer during discharge process.

Supplementary Figure 5. The average neutron transmission change ratio (Trt/Tr0) of the Operando neutron imaging cell with 16.7mg/cm2 cathode as a function of time and the corresponding charge/discharge curve

Supplementary Figure 6. Zoomed-in neutron transmission change (Trt/Tr0) for the thin cathode layer during charge and discharge process.

Supplementary Figure 7. Cycling stability of the composite cathode with the carbon nanofibers, the cells were initialized at C/10 for the first cycle and then cycled at 2C.

Supplementary Figure 8. Critical current density (CCD) test for the In-Li anode

Supplementary Figure 9. Voltage profile of the CCD test for the In-Li anode

Supplementary Figure 10. Rate and cycling performance of thin LCO cathode (3 mg/cm2 with 65 wt% of LCO).

Supplementary Figure 11. (left) dQ/dV curves of the ASSBs with 3 mg/cm2 LCO cathode from C/10 to 2C and (right) zoom-in dQ/dV curves.

Supplementary Figure 12. The rate performance of ASSBs with the 30 mg/cm2 three-layer cathode to the cell fail.

Supplementary Figure 13. The rate performance of ASSBs with the 100 mg/cm2 three-layer cathode to the cell fail.

Supplementary Figure 14. Charge/discharge profiles from cycle 34 to 43 of the battery with 30 mg/cm2 three-layer LCO cathode.

Supplementary Figure 15. Charge/discharge profiles from cycle 29 to 34 of the battery with 30 mg/cm2 three-layer LCO cathode.

Supplementary Table 1. Neutron attenuation coefficients for nature Li, Li isotopes, and other materials

| Material | Neutron attenuation coefficient, Σ [cm−1]* |
| --- | --- |
| Nature Li | 4.6964 |
| 6Li | 33.5047 |
| 7Li | 0.0543 |
| In | 10.3944 |
| Li5.4PS4.4Cl1.6 ** | 2.4385 |
| 6Li5.4PS4.4Cl1.6 | 27.4019 |
| LiNi0.8Mn0.1Co0.1O2** | 2.8689 |
| Li0.5Ni0.8Mn0.1Co0.1O2** | 1.8688 |

*All values are for cold neutrons at a wavelength of 2.53 Å

** Li element is nature Li

Supplementary Equation 1. Calculation of tortuosity of the composite cathode1

τi2=σi,effσi,0∅i

Where τi is the tortuosity factor,  σi,eff is the effective conductivity, σi,0 is the bulk conductivity, and  ϕi the volume fraction.

Reference

1	Minnmann, P., Quillman, L., Burkhardt, S., Richter, F. H. & Janek, J. Editors’ choice—quantifying the impact of charge transport bottlenecks in composite cathodes of all-solid-state batteries. Journal of The Electrochemical Society 168, 040537 (2021).