Table 1 Optimization of the reaction conditions for the Hantzsch condensation of para-Chlorobenzaldehyde, dimedone, ethyl acetoacetate and ammonium acetate as a model reaction for the synthesis of polyhydroquinolines.

| Entry | Catalyst | Amount of Catalyst (mg) | Solvent | Temperature (ºC) | Time (min) | Yield (%)a,b |
| --- | --- | --- | --- | --- | --- | --- |
|  | - | - | EtOH | reflux | 85 | 17 |
|  | 4,6-diamino-2-pyrimidinethiol | 7 | EtOH | reflux | 85 | 23 |
|  | Ag(NO3)2 | 7 | EtOH | reflux | 85 | Trace |
|  | Ag-CP | 4 | EtOH | reflux | 85 | 69 |
|  | Ag-CP | 5 | EtOH | reflux | 85 | 74 |
|  | Ag-CP | 6 | EtOH | reflux | 85 | 78 |
|  | Ag-CP | 7 | EtOH | reflux | 85 | 87 |
|  | Ag-CP | 7 | EtOH:H2O | 80 | 90 | 82 |
|  | Ag-CP | 7 | PEG-400 | 80 | 120 | 75 |
|  | Ag-CP | 7 | DMF | 80 | 110 | 74 |
|  | Ag-CP | 7 | DMSO | 80 | 125 | 78 |
|  | Ag-CP | 7 | EtOH | 25 | 8 h | NR |
|  | Ag-CP | 7 | EtOH | 60 | 70 | 76 |
|  | Ag-CP | 7 | EtOH | 70 | 75 | 79 |

a Isolated yield.

b Reaction conditions: 4-Chlorobenzaldehyde (1mmol), dimedone (1 mmol), ethyl acetoacetate (1 mmol), ammonium acetate (1.2 mmol), catalyst (mg) and solvent (3mL).

Table 2 Hantzsch synthesis of polyhydroquinoline derivatives in the presence of Ag-CP  in EtOH at 80 °C.

| Entry | Aryl aldehyde | Product | Time (min) | Yield (%)a,b | Melting point |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  | measured | literature |
| 1 |  |  | 80 | 93 | 198-205 | 203-206 54 |
| 2 |  |  | 85 | 87 | 245-248 | 246-247 54 |
| 3 |  |  | 80 | 86 | 245-249 | 249-251 54 |
| 4 |  |  | 86 | 82 | 249-251 | 252-255 42 |
| 5 |  |  | 80 | 83 | 254-256 | 255-257 42 |
| 6 |  |  | 85 | 87 | 197-202 | 204-206 54 |
| 7 |  |  | 85 | 88 | 264-268 | 246 – 248 55 |
| 8 |  |  | 80 | 93 | 169-174 | 175-176 54 |
| 9 |  |  | 80 | 87 | 208-210 | 230-232 32 |
| 10 |  |  | 85 | 81 | 238-240 | 231–233 42 |
| 11 |  |  | 85 | 74 | 294-295 | 305 - 307 56 |
| 12 |  |  | 90 | 78c | 298 = decomposition | 298-300 57 |

b Isolated yields.

b Reaction conditions: Aromatic aldehyde (1mmol), dimedone (1 mmol), ethyl acetoacetate (1 mmol), ammonium acetate (1.2 mmol), Ag-CP  (7 mg) and EtOH (3mL) at 80°C reflux conditions.

c Reaction conditions: Aromatic aldehyde (1mmol), dimedone (2 mmol), ethyl acetoacetate (2 mmol), ammonium acetate (2.4 mmol), Ag-CP  (14 mg) and EtOH (6mL) at 80°C reflux conditions.

Table 3. Comparison of the synthesis of polyhydroquinolines in the presence of various catalysts.

| Entry | Catalyst | Time (min) | Yield (%)a | Ref |
| --- | --- | --- | --- | --- |
|  | FeAl2O4 | 180 | 90 | 32 |
|  | Fe3O4@D-NH-(CH2)4-SO3H | 90 | 86 | 58 |
|  | Fe3O4@FSM-16-SO3H | 25 | 86 | 59 |
|  | AIL-SCMNPs | 15 | 80 | 60 |
|  | Ag-CP | 85 | 87 | This work |

a Isolated yield.