Supporting Information

Supplementary Fig. 1: OER overpotential at 10 mA/cm2 of Co3O4 into which we introduced increasing concentrations of octahedral Co2+.

Supplementary Fig. 2: O K-edge sXAS spectra for Co1.8Ga1.2O4 inverse spinel, Co3O4 normal spinel, and Ga2O3 metal oxide. We find out that in both Co3O4 and Ga2O3 only one prominent peak can be located around 529 eV, while a new peak at 528 eV can be found in Co1.8Ga1.2O4 mixed spinel. This new peak can be ascribed to the transition of electrons in t2g orbitals filling the eg orbitals, giving rise to the partially unoccupied t2g states and higher spine state of cobalt ions.

Supplementary Fig. 3: XPS spectra pf CoxGa(3-x)O4 with different concentration of Ga3+.

Supplementary Fig. 4: Electrochemical double layer capacitance of a, Co3O4 normal spinel and b, Co1.8Ga1.2O4 mixed spinel. c, the Electrochemical surface area (ECSA) comparison. Co3O4 normal spinel has an ECSA of 0.25 mF/cm2, while Co1.8Ga1.2O4 mixed spinel has an ECSA of 1.31 mF/cm2.

Supplementary Fig. 5: Tafel slopes comparison between Co3O4 normal spinel and Co1.8Ga1.2O4 mixed spinel.

Supplementary Fig. 6: Nyquist plots comparison between Co3O4 normal spinel and Co1.8Ga1.2O4 mixed spinel.

Supplementary Fig. 7: ICP-AES results of a, Co1.8Ga1.2O4 and b, Co3O4 working at 10 mA/cm2 in 0.5 M H2SO4, showing 5/6 of Co in Co1.8Ga1.2O4 inverse spinel can be protected against dissolution during 100 hours test.

Supplementary Fig. 8: a, XRD pattern of CoxGa(3-x)O4 after stability test. b, TEM image of Co1.8Ga1.2O4 after stability test. c, XPS spectra of Co in Co1.8Ga1.2O4 after stability test.

Supplementary Fig. 9: OER activity and stability for recently reported earth abundant electrocatalysts6,20-31

Supplementary Fig. 10: I-V curves of Co3O4 normal spinel and Co1.8Ga1.2O4 mixed spinel in PEMWE, categorized by kinetic overpotential (ηkinetics), ohmic overpotential (ηohmic), and mass transfer overpotential (ηmass transfer). PEMWE performance of Co3O4 normal spinel and Co1.8Ga1.2O4 mixed spinel at a, Initial stage, b, after working at 200 mA/cm2 for 12h, c, in a membrane electrode assembly washed using acid, then subjected to PEMWE evaluation. Comparison of cell voltage contributed by ηkinetics, ηohmic, and ηmass transfer using d, Co3O4 normal spinel and e, Co1.8Ga1.2O4 mixed spinel as the anode.

Supplementary Fig. 11: Surface structures of Co3O4 and Co1.8Ga1.2O4. (311) surface structures of Co3O4 (a), Co3O4 with one Co atom substituted by Ga atom (b), and Co3O4 with two Co atoms substituted by Ga atoms (c). The pink, purple, and red atoms refer to Co, Ga, and O, respectively. A and B sites labelled by black arrows represent the tetrahedral and octahedral site in the normal and inverse spinel structure. The location of substituted Ga atoms was determined by systematically consider the inequivalent site and used the most thermodynamic stable configuration as the final structure, and the structure in c was used to represent the Co1.8Ga1.2O4 in the present study.

Supplementary Fig. 12: OER intermediates in AEM on Co3O4. OER intermediates in AEM, *O, *OH, *OOH, adsorbed on A site (a) and B site (b), respectively. The pink and red atoms refer to Co and O, respectively.

Supplementary Fig. 13: OER intermediates in AEM on Co1.8Ga1.2O4. OER intermediates in AEM, *O, *OH, *OOH, adsorbed on A site (a) and B site (b), respectively. The pink, purple, and red atoms refer to Co, Ga, and O, respectively.

Supplementary Fig. 14: OER intermediates in OPM on Co3O4. OER intermediates in OPM, *OH-*O, *OH-*OH, *O-*O, adsorbed on combined A-B sites (a) and B-B sites (b), respectively. The pink and red atoms refer to Co and O, respectively.

Supplementary Fig. 15: OER intermediates in OPM on Co1.8Ga1.2O4. OER intermediates in OPM, *OH-*O, *OH-*OH, *O-*O, adsorbed on combined A-B sites (a) and B-B sites (b), respectively. The pink and red atoms refer to Co and O, respectively.

Supplementary Fig. 16: Co3O4 surfaces in dissolution pathways. Optimized geometry of Co3O4 surfaces in M and O pathways as depicted in Fig. 4c, respectively. R1’–R3’ is the M pathway which prioritizes metal dissolution. R4’–R6’ is the O pathway which prioritizes oxygen 6 dissolution. The pink, purple, and red atoms refer to Co, Ga, and O, respectively.

Supplementary Fig. 17: Co1.8Ga1.2O4 surfaces in dissolution pathways. Optimized geometry of Co1.8Ga1.2O4 surfaces in M and O pathways as depicted in Fig. 4c, respectively. R1’–R3’ is the M pathway which prioritizes metal dissolution. R4’–R6’ is the O pathway which prioritizes oxygen 6 dissolution. The pink, purple, and red atoms refer to Co, Ga, and O, respectively.

Supplementary Fig. 18: 	Energetics of dissolution on Co3O4 and Co1.8Ga1.2O4 surfaces. OER intermediates in AEM, *O, *OH, *OOH, adsorbed on A site (a) and B site (b), respectively. The pink, purple, and red atoms refer to Co, Ga, and O, respectively.

Supplementary Table 1: OER performance comparison between Co1.8Ga1.2O4 inverse spinel with other PGM-free acidic OER electrocatalysts.

| Catalyst | Overpotential @10 mA/cm2 (mV) | Stability (time @ current density) | Reference in main text |
| --- | --- | --- | --- |
| CoMnLaOx | 300 | 350 h @ 10 mA/cm2 | 6 |
| Co2MnO4 | 395 | 320 h @ 100 mA/cm2; 60 h @ 200 mA/cm2 | 11 |
| Ba-Co3O4 | 278 | 110 h @ 10 mA/cm2 | 20 |
| NiFeP | 540 | 30 h @ 10 mA/cm2 | 21 |
| CoFePbOx | 700 | 8 h @100 mA/cm2 | 22 |
| Ni2Ta | 570 | 66 h @ 10 mA/cm2 | 23 |
| Mn-doped FeP/Co3(PO4)2 | 390 | 8.3 h@5 mA/cm2 | 24 |
| Co3O4 | 360 | 40 h @ 10 mA/cm2 | 25 |
| Mn7.5O10Br3 | 290 | 500 h @ 10 mA/cm2 | 26 |
| ONPPGC/OCC | 470 | 10 h@ 10 mA/cm2 | 27 |
| Co3O4@C | 370 | 82 h @100 mA/cm2 | 28 |
| C-Fe3O4 | 650 | 24 h @ 10 mA/cm2 | 29 |
| CuMnO:F | 325 | 24 h @ 16 mA/cm2 | 30 |
| MnOx | 420 | 3200 h@200 mA/cm2 | 31 |
| Co1.8Ga1.2O4 | 270 | 200 h @ 200 mA/cm2 | This work |