Industrial lignins: the potential for efficient removal of Cr(VI) from wastewater

Hao Zhang, Haifeng Zhou*

Key Laboratory of Low Carbon Energy and Chemical Engineering, College of Chemical and Biological Engineering, Shandong University of Science and Technology, Qingdao, 277590, China

*Corresponding author: Haifeng Zhou

Phone: +86-532-86057766

E-mail: zhouhaifeng-qd@163.com

b

b

a

a

c

c

e

e

d

d

f

f

Fig.S1. The survey EDS spectra of ELN, BLN and FS before (a, c, e) and after (b, d, f) Cr(VI) adsorption.

Fig.S2. Effect of temperature on the adsorption of Cr(VI) by ELN (a), BLN (b), FS (c).

Fig.S3. Changes of Cr species in solution during ELN (a), BLN (b) and FS (c) adsorption process.

Fig. S4 .The plots of ln(Kd) versus 1/T.

Table S1 Fitting parameters of Langmuir isotherm model.

| Temperature /°C | Parameter | Materials |  |  |
| --- | --- | --- | --- | --- |
|  |  | ELN | BLN | FS |
|  | qe (exp) (mg g-1) | 626.03 | 735.40 | 466.84 |
| 25 | KL (L mg-1) | 0.0036 | 0.9283 | 0.0085 |
|  | qm (mg g-1) | 638.11 | 819.29 | 477.52 |
|  | R2 | 0.9970 | 0.9940 | 0.9146 |
|  | qe (exp) (mg g-1) | 639.80 | 761.14 | 509.55 |
| 35 | KL (L mg-1) | 0.0245 | 1.2956 | 0.0299 |
|  | qm (mg g-1) | 689.90 | 825.53 | 619.99 |
|  | R2 | 0.9846 | 0.9919 | 0.9654 |
|  | qe (exp) (mg g-1) | 723.93 | 791.23 | 588.59 |
| 45 | KL (L mg-1) | 0.0266 | 1.4252 | 0.0367 |
|  | qm (mg g-1) | 765.60 | 880.57 | 721.58 |
|  | R2 | 0.9969 | 0.9888 | 0.9459 |

Table S2 Fitting parameters of Freundlich isotherm model.

| Temperature /°C | Parameter | Materials |  |  |
| --- | --- | --- | --- | --- |
|  |  | ELN | BLN | FS |
| 25 | KF (L g-1) | 108.617 | 523.500 | 58.814 |
|  | 1/n | 0.2555 | 0.0504 | 0.2920 |
|  | R2 | 0.8347 | 0.9819 | 0.8702 |
| 35 | KF (L g-1) | 258.696 | 576.270 | 131.168 |
|  | 1/n | 0.1319 | 0.0417 | 0.1902 |
|  | R2 | 0.9491 | 0.9762 | 0.9627 |
| 45 | KF (L g-1) | 309.139 | 591.963 | 169.335 |
|  | 1/n | 0.1256 | 0.0425 | 0.1805 |
|  | R2 | 0.9384 | 0.9806 | 0.9414 |

Table S3 Fitting parameters of Pseudo-first-order dynamics model

| Materials | Parameter | Concentration (mg L-1) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | 600 | 800 | 1000 | 1200 | 1400 |
| FS | qe (exp) (mg g-1) | 379.72 | 417.04 | 443.93 | 463.37 | 482.82 |
|  | k1×10-4 (min-1) | 3.6090 | 4.5718 | 7.5761 | 5.8594 | 9.4919 |
|  | qe (mg g-1) | 313.24 | 304.78 | 300.96 | 262.09 | 240.26 |
|  | R2 | 0.8676 | 0.9324 | 0.9542 | 0.9160 | 0.9483 |
| BLN | qe (exp) (mg g-1) | 596.68 | 719.58 | 723.82 | 726.76 | 758.83 |
|  | k1×10-4 (min-1 ) | 4.9844 | 7.9332 | 8.3541 | 8.2580 | 11.2000 |
|  | qe (mg g-1) | 559.42 | 576.61 | 600.38 | 568.70 | 570.48 |
|  | R2 | 0.8260 | 0.9337 | 0.9550 | 0.9314 | 0.9642 |
| ELN | qe (exp) (mg g-1) | 509.78 | 574.62 | 589.21 | 601.86 | 626.16 |
|  | k1×10-4 (min-1 ) | 4.4841 | 6.2426 | 6.9176 | 7.4231 | 9.3641 |
|  | qe (mg g-1) | 481.65 | 466.68 | 479.39 | 444.20 | 426.19 |
|  | R2 | 0.9199 | 0.9547 | 0.9686 | 0.9507 | 0.9400 |

Table S4 Fitting parameters of Pseudo- second-order dynamics model

| Materials | Parameter | Concentration (mg L-1) |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | 600 | 800 | 1000 | 1200 | 1400 |
| FS | qe (exp) (mg g-1) | 379.72 | 417.04 | 443.93 | 463.37 | 482.82 |
|  | k2×10-5 (g/min-1 mg-1) | 1.4623 | 1.2247 | 1.2319 | 1.3140 | 1.5908 |
|  | qe (mg g-1) | 387.60 | 425.53 | 462.96 | 471.70 | 490.20 |
|  | R2 | 0.9974 | 0.9961 | 0.9980 | 0.9972 | 0.9989 |
| BLN | qe (exp) (mg g-1) | 596.68 | 719.58 | 723.82 | 726.76 | 758.83 |
|  | k2×10-6 (g/min-1 mg-1) | 4.9360 | 3.0566 | 3.2862 | 3.4471 | 3.6124 |
|  | qe (mg g-1) | 649.35 | 787.40 | 806.45 | 787.40 | 819.67 |
|  | R2 | 0.9982 | 0.9978 | 0.9964 | 0.9996 | 0.9997 |
| ELN | qe (exp) (mg g-1) | 509.78 | 574.62 | 589.21 | 601.86 | 626.16 |
|  | k2×10-6 (g/min-1 mg-1) | 5.5608 | 5.1397 | 4.6078 | 5.7277 | 6.0924 |
|  | qe (mg g-1) | 540.54 | 606.06 | 625.00 | 628.93 | 653.59 |
|  | R2 | 0.9972 | 0.9966 | 0.9955 | 0.9977 | 0.9989 |