Table IV: Molar refractivity (Rm), molar polarizability (αm), reflection loss (RL), metallization criteria (M), refractive index (no), optical electronegativity (χ), energy band gap based oxide ion polarizability (αo-2(Eg)), theoretical optical basicity (Ʌth), optical basicity (Ʌ) and theoretical interaction parameter (Ath) and energy gap based interaction parameter of A(Eg)
(70-x) B2O3 -10ZnO-10CdO-10MgO-xBi2O3 (x = 5, 10, 15, 20 and 25 mole %).

| Parameters | x=5 | x=10 | x=15 | x=20 | x=25 |
| --- | --- | --- | --- | --- | --- |
| Rm (cc/mol) | 17.401 | 19.444 | 20.759 | 22.140 | 22.897 |
| αm (Å3) | 6.894 | 7.703 | 8.224 | 8.771 | 9.071 |
| RL | 0.630 | 0.635 | 0.641 | 0.645 | 0.650 |
| M | 0.369 | 0.364 | 0.358 | 0.354 | 0.349 |
| no | 2.473 | 2.495 | 2.526 | 2.543 | 2.566 |
| χ | 0.733 | 0.715 | 0.688 | 0.674 | 0.655 |
| αo-2(Eg) (Å3) | 2.816 | 3.028 | 3.183 | 3.348 | 3.411 |
| Ʌth | 0.542 | 0.589 | 0.637 | 0.684 | 0.731 |
| Ʌ (Eg) | 1.077 | 1.118 | 1.145 | 1.172 | 1.180 |
| Ath (Å-3) | 0.207 | 0.193 | 0.178 | 0.163 | 0.148 |
| A (Eg) (Å-3) | 0.08518 | 0.08312 | 0.08106 | 0.079 | 0.07694 |