Table I. Average molecular weight MW, experimental density ρ, molar volume Vm, oxygen packing density OPD, oxygen molar Volume Vo, Bi3+ ion concentration NBi, polaron radius rp, inter ionic distance ri Field strength Fs and boron-boron distance dB-B, theoretical density ρth,, cross-link density nc, bond density nb and co-ordination number of glass m of                                   (70-x)B2O3 -10ZnO-10CdO-10MgO-xBi2O3  (x = 5, 10, 15, 20 and 25 mole %) glasses.

| Physical Parameters | X = 5 | X = 10 | X = 15 | X = 20 | X = 25 |
| --- | --- | --- | --- | --- | --- |
| MW (g/mol) | 93.561 | 113.378 | 133.195 | 153.012 | 172.829 |
| ρ (g/cc) | 3.38 | 3.70 | 4.11 | 4.46 | 4.91 |
| Vm (cc/mol) | 27.60 | 30.60 | 32.33 | 34.29 | 35.19 |
| OPD (g.atm/l) | 86.93 | 78.40 | 74.22 | 69.98 | 68.18 |
| Oxygen molar volume Vo (cc/mol) | 11.50 | 12.75 | 13.47 | 14.28 | 14.66 |
| NBi (*1021 ions/cc) | 1.09 | 1.96 | 2.79 | 3.51 | 4.27 |
| rp (Å) | 3.91 | 3.21 | 2.86 | 2.65 | 2.48 |
| ri (Å) | 9.71 | 7.97 | 7.10 | 6.57 | 6.16 |
| Field strength Fs (*1016 cm-2) | 5.41 | 8.02 | 10.14 | 11.81 | 13.47 |
| VmB | 39.43 | 38.26 | 35.92 | 34.29 | 31.99 |
| dB-B (A0) | 4.03 | 3.99 | 3.90 | 3.84 | 3.75 |
| ρth (g/cc) | 2.86 | 3.41 | 3.95 | 4.47 | 4.98 |
| Cross-link Density nc | 1.70 | 1.88 | 2.05 | 2.23 | 2.41 |
| Bond density nb (*1022) (cc-1) | 10.25 | 9.44 | 9.12 | 8.78 | 8.72 |
| Coordination no. of glass m | 4.7 | 4.8 | 4.9 | 5.0 | 5.1 |