Table III: Cut-off wavelength λc, indirect optical band gap energy Eg , direct optical band gap Eg  and Urbach energy ΔE for Tauc and ASF model of the present glasses (70-x)B2O3 -10ZnO-10CdO-10MgO-xBi2O3 for x= 5, 10, 15, 20 and 25 mol%.

|  |  | Tauc model |  |  | ASF model |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Bi2O3 content | Cut- off wavelength λc (nm) | (Eg) (eV) indirect | (Eg) (eV) direct | ΔE (eV) | (Eg) (eV) indirect | (Eg) (eV) direct | ΔE (eV) |
| X=5 | 387 | 2.73 | 3.21 | 0.33 | 2.78 | 3.21 | 0.34 |
| X=10 | 395 | 2.66 | 3.19 | 0.28 | 2.66 | 3.15 | 0.30 |
| X=15 | 404 | 2.56 | 3.08 | 0.25 | 2.56 | 3.08 | 0.27 |
| X=20 | 414 | 2.51 | 2.95 | 0.24 | 2.52 | 2.99 | 0.24 |
| X=25 | 426 | 2.44 | 2.84 | 0.23 | 2.49 | 2.84 | 0.20 |
| Earlier work [ref] |  |  |  |  |  |  |  |
| (20 + x) Bi2O3–20BaO–10Na2O–10MgO–(40-x) B2O3 (where x = 0, 5, 10, 15 and 20 mol%) [49] |  |  |  |  |  |  |  |
| X=0 |  | 2.661 | 2.905 |  |  |  |  |
| X=5 |  | 2.628 | 2.886 |  |  |  |  |
| X=10 |  | 2.601 | 2.866 |  |  |  |  |
| X=15 |  | 2.568 | 2.833 |  |  |  |  |
| X=20 |  | 2.536 | 2.806 |  |  |  |  |
| 20Li2O-(20-x) Bi2O3-xWO3-60B2O3 (x= 0, 1, 2, 3, 4 and 5 mol %) [50] |  |  |  |  |  |  |  |
| X=0 |  |  |  |  | 2.96 | 3.359 |  |
| X=1 |  |  |  |  | 2.901 | 3.322 |  |
| X=2 |  |  |  |  | 2.851 | 3.31 |  |
| X=3 |  |  |  |  | 2.839 | 3.223 |  |
| X=4 |  |  |  |  | 2.653 | 3.119 |  |
| X=5 |  |  |  |  | 2.616 | 3.074 |  |
| xBi2O3-(80-x) TeO2-10B2O3-10GeO2 [51] |  |  |  |  |  |  |  |
| X=40 |  | 3.07 |  |  |  |  |  |
| X=45 |  | 3.01 |  |  |  |  |  |
| X=50 |  | 2.91 |  |  |  |  |  |
| X=55 |  | 2.88 |  |  |  |  |  |
| X=60 |  | 2.86 |  |  |  |  |  |
| X=65 |  | 2.81 |  |  |  |  |  |
| 50Bi2O3-20B2O3-15Li2O-15MO (Where MO = ZnO, CdO, BaO, and PbO) [52] |  |  |  |  |  |  |  |
| ZnO |  | 1.931 | 2.131 |  |  |  |  |
| CdO |  | 1.7469 | 1.971 |  |  |  |  |
| BaO |  | 1.605 | 1.763 |  |  |  |  |
| PbO |  | 1.415 | 1.545 |  |  |  |  |