Tables

| Table 1: Codes and actual variables and their levels in BBD |  |  |  |  |
| --- | --- | --- | --- | --- |
| Codes | Variables | Level 1 (-1) | Level 2 (0) | Level 3 (+1) |
| A | CHS-GLU/BCL Dose (g/100 mL) | 0.02 | 0.06 | 0.1 |
| B | Contact time (min) | 5 | 17.5 | 30 |
| C | Solution pH | 4 | 7 | 10 |

Table 2: Experimental matrix based on BBD approach for designing experiments and the corresponding response (AR88 removal (%)).

| Run | A: CHS-GLU/BCL dose (g) | B: Time (min) | C: pH | AR88 removal (%) |
| --- | --- | --- | --- | --- |
| 1 | 0.02 | 5 | 7 | 8.3 |
| 2 | 0.1 | 5 | 7 | 36.7 |
| 3 | 0.02 | 30 | 7 | 21.0 |
| 4 | 0.1 | 30 | 7 | 84.7 |
| 5 | 0.02 | 17.5 | 4 | 24.6 |
| 6 | 0.1 | 17.5 | 4 | 92.1 |
| 7 | 0.02 | 17.5 | 10 | 5.1 |
| 8 | 0.1 | 17.5 | 10 | 19.4 |
| 9 | 0.06 | 5 | 4 | 39.0 |
| 10 | 0.06 | 30 | 4 | 91.2 |
| 11 | 0.06 | 5 | 10 | 7.3 |
| 12 | 0.06 | 30 | 10 | 16.5 |
| 13 | 0.06 | 17.5 | 7 | 42.0 |
| 14 | 0.06 | 17.5 | 7 | 36.8 |
| 15 | 0.06 | 17.5 | 7 | 33.0 |
| 16 | 0.06 | 17.5 | 7 | 40.0 |
| 17 | 0.06 | 17.5 | 7 | 37.5 |

Table 3: Analysis of variance (ANOVA) for AR88 dye removal onto CHS-GLU/BCL

| Source | Sum of Squares | df | Mean Square | F-value | p-value | Remark |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 12049.26 | 6 | 2008.21 | 183.81 | < 0.0001 | significant |
| A-Dose | 3779.71 | 1 | 3779.71 | 345.95 | < 0.0001 | significant |
| B-Time | 1859.95 | 1 | 1859.95 | 170.24 | < 0.0001 | significant |
| C-pH | 4929.50 | 1 | 4929.50 | 451.18 | < 0.0001 | significant |
| AB | 311.30 | 1 | 311.30 | 28.49 | 0.0003 | significant |
| AC | 707.82 | 1 | 707.82 | 64.79 | < 0.0001 | significant |
| BC | 460.98 | 1 | 460.98 | 42.19 | < 0.0001 | significant |
| Residual | 109.26 | 10 | 10.93 |  |  |  |
| Lack of Fit | 62.56 | 6 | 10.43 | 0.8930 | 0.5716 | not significant |
| Pure Error | 46.70 | 4 | 11.68 |  |  |  |
| Cor Total | 12158.51 | 16 |  |  |  |  |
| R² | 0.9910 |  | Predicted R² | 0.9696 |  |  |
| Adjusted R² | 0.9856 |  | Adeq Precision | 43.9024 |  |  |

| Table 4: PFO and PSO kinetic parameters for CHS-GLU/BCL adsorption on AR88 dye |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PSO |  |  |  |  | PFO |  |  |  | qe exp. (mg/g) | Concentration (mg/L) |
| R2 | k2 × 10-2 (g/mg min) |  |  | qe cal (mg/g) | R2 | k1 (1/min) | qe cal (mg/g) |  |  |  |
| 0.99 |  |  | 0.68 | 48 |  | 0.99 | 0.19 |  | 46 | 46 | 20 |
| 0.99 |  |  | 0.96 | 61 |  | 0.97 | 0.30 |  | 59 | 60 | 40 |
| 0.99 |  |  | 0.06 | 120 |  | 0.99 | 0.06 |  | 117 | 117 | 60 |
| 0.99 |  |  | 0.04 | 133 |  | 0.99 | 0.03 |  | 135 | 132 | 80 |
| 0.99 |  |  | 0.02 | 142 |  | 0.99 | 0.03 |  | 139 | 137 | 100 |
| 0.99 |  |  | 0.02 | 164 |  | 0.99 | 0.02 |  | 160 | 165 | 150 |

Table 5: The parameters of isotherm models for CHS-GLU/BCL dye adsorption on AR88

| Adsorption isotherm | Parameter | Value |
| --- | --- | --- |
| Langmuir | qmax (mg/g) | 148 |
|  | Ka (L/mg) | 3.60 |
|  | R2 | 0.98 |
| Freundlich | Kf (mg/g) (L/mg)1/n | 99 |
|  | n | 5.62 |
|  | R2 | 0.90 |
| Temkin | KT (L/mg) | 120 |
|  | bT (J/mol) | 116 |
|  | R2 | 0.92 |

Table 6: Comparison of The Adsorption Capacity of AR88 on CHS-GLU/BCL with different Adsorbents.

| Adsorbents | qmax (mg/g) | References |
| --- | --- | --- |
| CHS-GLU/BCL | 148 | This study |
| Zeolite/Chitosan Hydrogel | 332.48 | [59] |
| Hexadecyltrimethylammonium (HDTMA)-bentonite | 91.70 | [60] |
| Nitrogen-containing Graphitic Mesoporous Carbon | 309 | [61] |
| Phosphorylated chitosan (P-CS) | 230 | [62] |
| Bio-Silica/Chitosan | 25.84 | [63] |

Table 7: Thermodynamic parameters for the adsorption of AR88 on CHS-GLU/BCL.

| T (K) | kd | ∆Go (kJ/mol) | ∆Ho (kJ/mol) | ∆So (kJ/molK) |
| --- | --- | --- | --- | --- |
| 298.15 | 30.5 | -8.21 | - 39.2 | - 0.11 |
| 308.15 | 21.3 | -7.17 |  |  |
| 318.15 | 9.02 | -6.13 |  |  |
| 328.15 | 6.31 | -5.09 |  |  |