SUPPLEMENTARY MATERIALS

Immobilization of Bacillus subtilis in biohybrid crosslink chitosan-glutaraldehyde for acid red 88 dye removal: Box–Behnken design optimization and mechanism study

Hasan M. Aghaa,b, Abdulmutalib Allaqc, Ali H. Jawada,b,e*, Shafiq Aazmid,  Zeid A. ALOthmane, Lee D. Wilsonf

aFaculty of Applied Sciences, Universiti Teknologi MARA, 40450 Shah Alam, Selangor, Malaysia

bAdvanced Biomaterials and Carbon Development Research Group, Faculty of Applied Sciences, Universiti Teknologi MARA, 40450 Shah Alam, Selangor, Malaysia

cFaculty of Applied Science, Department Applied Microbiology, Universiti Teknologi MARA, Shah Alam 40450, Malaysia

dMicrobiome Health and Environment (MiHeaRT) Research Group, Faculty of Applied Sciences, Universiti Teknologi MARA, Shah Alam, Selangor, Malaysia

eEnvironmental and Atmospheric Sciences Research Group, Scientific Research Center, Al-Ayen University, Thi-Qar, Nasiriyah, 64001, Iraq

eChemistry Department, College of Science, King Saud University, Riyadh 11451, Saudi Arabia

fDepartment of Chemistry, University of Saskatchewan, Saskatoon, SK S7N 5C9, Canada

Corresponding author:

E-mail: ali288@uitm.edu.my; ahjm72@gmail.com (Ali H. Jawad)

Text S1

The FE-SEM (Field Emission Scanning Electron Microscopy) was used to evaluate the surface morphologies of the CHS-GLU/BCL bioadsorbent before and after biosorption of AR88 dye. The physical parameters of the CHS-GLU/BCL bioadsorbent were also analyzed. The elemental composition of the CHS-GLU/BCL bioadsorbent was determined using energy dispersive X-ray (EDX) analysis, both prior to and after AR88 dye biosorption. Utilizing a PANalytical X'Pert PRO diffractometer. X-ray diffraction (XRD) patterns were obtained for CHS, and CHS-GLU/BCL bioadsorbent in the range of 5° to 90° of 2-theta. The surface charge of the CHS-GLU/BCL bioadsorbent was determined using pHpzc [31]. The CHS-GLU/BCL bioadsorbent was analyzed using KBr pellets and a Perkin-Elmer Spectrum RX I spectrometer, which has a wavenumber range of 4000 cm-1 to 450 cm-1. FTIR spectra were determined before and after the biosorption of AR88 dye.

Fig. S1: Desirability tool of AR88 removal (%) by CHS-GLU/BCL biosorbent.

pHpzc

Fig. S2: pHpzc of CHS-GLU/BCL biosorbent

Table S1: Adsorption kinetics and isotherms nonlinear models

| Models | Formula | Descriptions |
| --- | --- | --- |
| Pseudo-first order (PFO) | qt=qe1-e-k1t | k1: pseudo-first-order rate constant (1/min) |
| Pseudo-second order (PSO) | qt=qe2k2t1+ qeK2t | k2: pseudo-second-order rate constant (g/mg min) |
| Langmuir | qe=qmKLCe1+ KLCe | qm : monolayer capacity (mg/g) KL: Langmuir constant (L/mg) |
| Freundlich | qe=KFCe1n | KF : Freundlich constant (mg/g) (L/mg)1/n n: adsorption intensity |
| Temkin | qe=RTbTlnKTCe | KT: Temkin constant (L/mg) : Heat of adsorption (J/mol) |