Supporting Information

Investigating the Electrochemical Properties of Ionic-Liquid-Mediated Inorganic Eutectogels Derived from Carboxylic-Acid-Based Hydrophobic Natural Deep Eutectic Solvents

Arindam Duttaa,b, Debashis Kunduc, Surbhi Sharmab, Debbie S. Silvesterb, Tamal Banerjeea*

aDepartment of Chemical Engineering, Indian Institute of Technology Guwahati, Guwahati, Assam 781039, India

bSchool of Molecular and Life Sciences, Curtin University, Perth, Western Australia 6845, Australia

cDepartment of Chemical Engineering, Institute of Chemical Technology Marathwada Campus, Jalna, Maharashtra 431203, India

*Corresponding author: Prof. Tamal Banerjee, tamalb@iitg.ac.in, + 91 361 258 2266

Fig. S1. 1H NMR spectra of (a) DES1, (b) DES2, (c) DES3, and (d) DES4.

Fig. S2. Images of (a) the coin cell assembly and (b) a piece of exfoliated rGO sheet used as electrode for the electrochemical experiments.

Fig. S3. Equivalent electrical circuit associated with a standard Nyquist plot derived from EIS.

Table S1. Water content in DESs 1 – 4.

| DES | Water content (wt%) |
| --- | --- |
| DES1 | 0.092 |
| DES2 | 0.086 |
| DES3 | 0.075 |
| DES4 | 0.061 |

Table S2. Rs, Rct, ESR, and ionic conductivity of Gels 1 – 4.

| Gel | Rs (Ω) | Rct (Ω) | ESR (Ω) = Rs + Rct | σ (mS cm-1) |
| --- | --- | --- | --- | --- |
| 1 | 16.05 | 69.92 | 85.97 | 15.87 |
| 2 | 15.64 | 51.35 | 66.99 | 16.28 |
| 3 | 17.47 | 107.47 | 124.94 | 14.58 |
| 4 | 17.52 | 118.4 | 135.92 | 14.53 |