Table Captions

Table 1. Archimedes results of the sintered PLZT samples.

Table 2. Miller indices, 2 angle, FWHM, interplaner distance, lattice constants (𝑎 and 𝑐), average crystal sizes (D), dislocation density and texturing coefficient () values ​​of PLZT materials exposed to sintering process at 1250 °C for 4 hours.

Table 3. Critical forces, depths and hardnesses and moduli of elasticity of PLZT materials with 2, 8 and 15 % La mole additions

Table 1. Archimedes results of the sintered PLZT samples.

| Material properties | Composition of PLZT materials |  |  |
| --- | --- | --- | --- |
|  | (2/65/35) | (8/65/35) | (15/65/35) |
| Weight loss (%) | 1.20 | 4.50 | 5.70 |
| Bulk density (gr/cm3) | 7.68 | 7.50 | 7.26 |
| Apparent specific gravity (gr/cm3) | 7.69 | 7.58 | 7.27 |
| Appa rent porosity (%) | 0.10 | 1.00 | 0.10 |
| Water absorption (%) | 0.00 | 0.10 | 0.00 |
| Linear shrinkage (on diameter) (%) | 14.50 | 17.10 | 17.40 |
| Linear shrinkage (on thickness) (%) | 12.00 | 17.10 | 13.40 |
| Linear volumetric shrinkage (%) | 36.00 | 43.00 | 41.00 |

Table 2. Miller indices, 2 angle, FWHM, interplaner distance, lattice constants (𝑎 and 𝑐), average crystal sizes (D), dislocation density and texturing coefficient () values ​​of PLZT materials exposed to sintering process at 1250 °C for 4 hours.

| PLZT materials | (hkl) | 2 (o) | FWHM (o) | d (Å) | TC | a (Å) | c (Å) | D (nm) | (1/nm3x10-4) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (2/65/35) | 110 | 31.70 | 0.550 | 3.3495 | 0.92 | 4.737 | 3.185 | 26.9 | 13.81 |
| (8/65/35) | 110 | 31.70 | 0.500 | 3.3495 | 0.89 | 4.737 | 3.185 | 28.7 | 12.14 |
| (15/65/35 | 110 | 31.70 | 0.450 | 3.3495 | 0.82 | 4.737 | 3.185 | 31.8 | 9.88 |

Table 3. Critical forces, depths and hardnesses and moduli of elasticity of PLZT materials with 2, 8 and 15 % La mole additions

| Sample name | SEQ | Force 1 (mN) | Depth 1 (m) | Depth 2 (m) | Depth 3 (m) | Depth 4 (m) | DHV-1 | DHV-2 | Elasticity Modulus (GPa) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| PLZT (2% La) | 1 | 999,70 | 4,843 | 3,928 | 4,308 | 0,535 | 164,488 | 250,047 | 77,5 |
|  | 2 | 750,17 | 3,761 | 3,123 | 3,328 | 0,433 | 204,627 | 296,856 | 88,1 |
|  | 3 | 501,00 | 3,121 | 2,732 | 2,881 | 0,240 | 198,411 | 259,004 | 124,0 |
|  | 4 | 250,50 | 2,120 | 1,998 | 2,025 | 0,095 | 215,102 | 242,193 | 118,0 |
|  | Average | 625,34 | 3,461 | 2,945 | 3,135 | 0,326 | 195,657 | 262,025 | 119,4 |
|  | Std.Dev. | 322,33 | 1,142 | 0,804 | 0,950 | 0,196 | 21,981 | 24,215 | 49,88 |
| PLZT (8% La) | 1 | 1000,2 | 3,284 | 2,358 | 2,577 | 0,707 | 357,894 | 693,816 | 95,4 |
|  | 2 | 750,6 | 2,646 | 1,917 | 2,097 | 0,549 | 413,507 | 787,999 | 113,0 |
|  | 3 | 499,5 | 2,515 | 2,015 | 2,153 | 0,362 | 304,772 | 474,478 | 114,0 |
|  | 4 | 250,1 | 1,727 | 1,622 | 1,665 | 0,063 | 323,477 | 366,972 | 278,0 |
|  | Average | 625,1 | 2,543 | 1,978 | 2,123 | 0,420 | 349,913 | 580,816 | 150,1 |
|  | Std.Dev. | 322,9 | 0,639 | 0,304 | 0,373 | 0,277 | 47,765 | 193,848 | 85,69 |
| PLZT (15% La) | 1 | 997,04 | 3,860 | 2,579 | 2,828 | 1,032 | 258,213 | 578,232 | 57,2 |
|  | 2 | 751,18 | 2,896 | 1,899 | 2,143 | 0,753 | 345,505 | 803,878 | 80,1 |
|  | 3 | 499,85 | 2,874 | 2,250 | 2,399 | 0,474 | 233,571 | 381,049 | 75,7 |
|  | 4 | 250,34 | 1,471 | 1,101 | 1,169 | 0,302 | 446,415 | 796,709 | 129,0 |
|  | Average | 624,60 | 2,775 | 1,957 | 2,135 | 0,640 | 320,938 | 633,967 | 85,5 |
|  | Std.Dev. | 321,65 | 0,984 | 0,635 | 0,703 | 0,321 | 96,468 | 201,895 | 30,65 |