Waterborne Polyurethane Modified with the Hydroxy Silicone Oils for Improving its Thermal, Water Resistance, and Mechanical Properties

Chao Liu1, Yujie Wang1, Wenli Li1, Yingchun Luo1, Wei Yan2, Guoyong Zhou1,*

1School of Chemical Engineering, Guizhou Minzu University, Guiyang 550025, PR China

2School of Materials Science and Engineering, Guiyang University, Guiyang 550005, PR China

Table S1 Performance characterization of waterborne polyurethane emulsion

| Sample | Particle size（nm） | PDI | Viscosity (mPas) | Mechanical stability |
| --- | --- | --- | --- | --- |
| 1% (Mn = 3000) | 61.97 | 0.087 | 23.2 | * |
| 5% (Mn = 3000) | 69.40 | 0.094 | 25.5 | * |
| 9% (Mn = 3000) | 82.53 | 0.148 | 28.7 | * |
| 13% (Mn = 3000) | 87.62 | 0.106 | 31.4 | * |
| 17% (Mn = 3000) | 92.37 | 0.135 | 37.2 | * |
| 1% (Mn = 10000) | 73.82 | 0.089 | 23.7 | * |
| 5% (Mn = 10000) | 82.09 | 0.159 | 26.5 | * |
| 9% (Mn = 10000) | 87.94 | 0.820 | 31.3 | * |
| 13% (Mn = 10000) | 94.35 | 0.190 | 33.4 | * |
| 17% (Mn = 10000) | 97.44 | 0.141 | 36.8 | * |
| 1% (Mn = 25000) | 75.14 | 0.078 | 25.5 | * |
| 5% (Mn = 25000) | 82.67 | 0.093 | 29.6 | * |
| 9% (Mn = 25000) | 91.70 | 0.016 | 35.7 | * |
| 13% (Mn = 25000) | 96.16 | 0.046 | 45.0 | * |
| 17% (Mn = 25000) | 103.27 | 0.138 | 47.6 | * |

Ps: The molecular weight of the hydroxy silicone oil added to the modification is in parentheses，* indicates that emulsion stable (>6 months).

Fig. S1 Morphology and particle size of Si-WPU emulsion

Fig. S2 Si 2p spectrum of Si-WPU (3000、10000、25000) surface (b)、(d)、(f)

Table S2 Elemental composition of film surface

| sample | mole fraction % |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | C | N | O | Si（actual） | Si（theory） |
| 1% (Mn=3000) | 56.71 | 1.18 | 23.37 | 18.73 | 0.32 |
| 5% (Mn=3000) | 62.46 | 1.13 | 23.15 | 13.26 | 1.61 |
| 9% (Mn=3000) | 66.61 | 0.79 | 22.78 | 9.82 | 2.88 |
| 13% (Mn=3000) | 57.48 | 0.85 | 24.15 | 17.50 | 4.17 |
| 17% (Mn=3000) | 53.14 | 0.72 | 23.84 | 22.29 | 5.44 |
| 1% (Mn=10000) | 52.77 | 1.35 | 25.08 | 20.78 | 0.53 |
| 5% (Mn=10000) | 69.98 | 1.57 | 19.47 | 8.96 | 1.59 |
| 9% (Mn=10000) | 52.17 | 1.32 | 25.04 | 21.47 | 4.76 |
| 13% (Mn=10000) | 51.73 | 0.94 | 24.69 | 22.63 | 6.89 |
| 17% (Mn=10000) | 55.21 | 0.61 | 25.17 | 19.01 | 8.26 |
| 1% (Mn=25000) | 60.24 | 1.58 | 23.16 | 15.02 | 0.67 |
| 5% (Mn=25000) | 52.82 | 1.27 | 23.73 | 22.17 | 3.35 |
| 9% (Mn=25000) | 51.60 | 0.74 | 24.94 | 22.71 | 6.02 |
| 13% (Mn=25000) | 61.79 | 0.83 | 21.45 | 15.91 | 7.71 |
| 17% (Mn=25000) | 50.59 | 0.66 | 25.00 | 23.75 | 8.79 |

Fig. S3 SEM images of the fracture surfaces of the WPU film surface (a),

the WPU film brittle fracture section (b)

* Corresponding authors.

E-mail address: gyzhou@gzmu.edu.cn.