Supporting Information

for

Fluorescence/colorimetric dual-signal sensor based on carbon dots and gold nanoparticles for visual quantization of Cr3+

Jinyu Shia,b, Suyi Wua, Yu Xuea, Qing Xieb, Qunzeng Danzengb, Cui Liub,*, Chuan-Hua Zhoua, **

a National Demonstration Center for Experimental Chemistry and Chemical Engineering Education (Yunnan University), School of Chemical Science and Technology, Yunnan University, Kunming 650091, China.

b Chongqing Key Laboratory of Natural Product Synthesis and Drug Research, Innovative Drug Research Center, School of Pharmaceutical Sciences, Chongqing University, Chongqing, 400044, P. R. China.

*Corresponding author: Cui Liu, E-mail addresses: liucui@cqu.edu.cn.

**Corresponding author: Chuan-Hua Zhou, E-mail addresses: chzhou@ynu.edu.cn.

Fig. S1. The relationship between I630nm/I518nm and pH of buffer (A), the relationship between (F/F0)/F0 and pH of buffer (B).

Fig. S2. The relationship between I630nm/I518nm and reaction time (A), the relationship between (F/F0)/F0 and reaction time (B).

Fig. S3. The relationship between fluorescence intensity of CD and dilution ratio (A), fluorescence spectra of CDs with different dilution ratio (B).

Fig. S4. UV-vis spectra of GSH-Au NPs with various temperatures (25℃, 60℃, 80℃).

Fig. S5. The relationship between I630nm/I518nm and GSH-Au NPs concentration (A), the relationship between (F/F0)/F0 and GSH-Au NP concentration (B).

Table S1. Fluorescence lifetimes of CDs and CDs+GSH-Au NPs

| Samples | CDs | CDs+GSH-Au NPs |
| --- | --- | --- |
| τ(ns) | 1.737 | 1.740 |