Supplementary Information

g-C3N4@COF heterojunction filler for polymer electrolytes enables fast Li+ transport and high mechanical strength

Experiment

Preparation of LiFePO4 cathode and the LiFePO4//Li cell assembly

Commercial LiFePO4, super-P, LiTFSI and PVDF were mixed in N-methyl pyrrolidone (NMP) with a mass ratio of 7:1:1:1 to form a uniform slurry, which was subsequently coated on Al foil. The prepared electrode films were dried at 120 °C for 24 h under vacuum before cell fabrication, and the active material loading of the LiFePO4 cathode is ~2 mg cm-2. Finally, different electrolytes were sandwiched between LiFePO4 cathode and Li metal anode to assemble the LiFePO4//Li cell. Electrochemical tests of the LiFePO4//Li battery was tested at room tempurature. (The theoretical capacity of LiFePO4 cathode is 170 mA g-1).

Materials Characterization

The overall morphology and nanostructure were investigated by Field Emission Scanning Electron Microscope (FSEM JEOL JSM-7100FA). Crystallographic characterization was conducted by D8 Discover X-ray diffractometer using Cu-Kα X-ray source with radiation (λ = 1.5418 Å). Stress-Strain curves were tested by Instron 5967.

Electrochemical Measurements

Ionic conductivity was determined by EIS after placing electrolyte membranes between two electrodes (stainless steel) in a CR2016 coin cell. The bulk resistance of the samples was calculated from the EIS curve. The ionic conductivity was obtained using Equation (1):

σ = LARb (1)

where A and L represent the area and thickness of the electrolyte membrane pellets, respectively. Rb is the bulk resistance, and σ is the ionic conductivity (S cm-1).

The Li-ion transference number (tLi+) was tested in symmetric lithium cell by a combination of DC polarization and AC impedance measurement. A DC potential (ΔV=10 mV) was applied for 5500 s to gain the initial and steady currents. Meanwhile, the AC impedance spectra of the same cell were measured before and after polarization. The value of lithium transference number (tLi+) have been calculated by equation (2):

tLi+=Is∆V-I0R0I0∆V-IsRs   (2)

Where R0 and RS are the AC impedances before and after polarization, respectively, I0 and IS are the initial and steady currents, respectively.

The cycle performances and rate performances of cells with solid electrolytes were measured by LiFePO4//Li batteries using a LANHE CT2001A charge/discharge system.

Results and Discussions

Figure S1. SEM images of the as-prepared g-C3N4

Figure S2. SEM images of PEO-LiTFSI electrolytes based on g-C3N4@COF composites with different C3N4/COF ratios: (a, b) g-C3N4/COF=1: 1,

(c, d) g-C3N4/COF=1.5: 1, (e, f) g-C3N4/COF=2: 1.

Figure S3. (a) Charge and discharge voltage profiles at the first cycle of LiFePO4//Li batteries assembled with PEO-LiTFSI electrolytes based on

g-C3N4@COF composites with different C3N4/COF ratios, (b) Cycling performance of LiFePO4//Li batteries assembled with PEO-LiTFSI electrolytes based on

g-C3N4@COF composites with different C3N4/COF ratios.

Figure S4. SEM images of PEO-LiTFSI-g-C3N4@COF (1.5:1) electrolytes with different SN addition amounts: (a, b) PEO: LiTFSI: g-C3N4@COF: SN=8: 1: 1:1, (c, d) PEO: LiTFSI: g-C3N4@COF: SN=8: 1: 1:1.5, (e, f) PEO: LiTFSI: g-C3N4@COF: SN=8: 1: 1: 2.

Figure S5. XRD patterns of PEO-LiTFSI-g-C3N4@COF (1.5:1) electrolytes with different SN addition amounts.

Figure S6. LSV curves of PEO-LiTFSI-g-C3N4@COF (1.5:1) electrolytes with different SN addition amounts: (a) 60 ℃, (b) 30 ℃

Figure S7. EIS patterns of PEO-LiTFSI-g-C3N4@COF (1.5:1) electrolytes with different SN addition amounts: (a) 30 ℃, (b) 60 ℃

Figure S8. EIS profiles and I-t curves of PEO-LiTFSI-g-C3N4@COF (1.5:1)-SN (8:1:1:2) electrolyte: (a) 60 ℃, (b) 30 ℃

Figure S9. (a) Charge and discharge voltage profiles at the first cycle of LiFePO4//Li batteries assembled with PEO-LiTFSI-g-C3N4@COF (1.5:1) electrolytes with different SN addition amounts, (b) Cycling performance of LiFePO4//Li batteries assembled with PEO-LiTFSI-g-C3N4@COF (1.5:1) electrolytes with different SN addition amounts