Table 1

Constituents of alginate-based active-intelligent films

| First layer Second layer |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Treatments | Compounds | SA (g) | M (g) | Gly (%) | W (mg/mL) | SA (g) | M (g) | Gly (%) | C3N4U (mg/mL) | C3N4FG (mg/mL) |
| A B C D | SA+W/ SA+ C3N4U SA+W/ SA+ C3N4FG SA+M+W/ SA+M +C3N4U SA+M+W/ SA+M +C3N4FG | 1 1 1 1 | 0 0 0.25 0.25 | 0.35 0.35 0.5 0.5 | 0.1 0.1 0.1 0.1 | 1 1 1 1 | 0 0 0.25 0.25 | 0.35 0.35 0.5 0.5 | 5 5 5 5 | 0 5 0 5 |

A, B, C, and D represent the films containing urea quantum dots, gelatin quantum dots, urea quantum dots and mucilage, and gelatin quantum dots and mucilage. SA, M, Gly, W, C3N4U, and C3N4FG are respectively the abbreviations of sodium alginate, mucilage, glycine, watercress, urea quantum dots, and fish gelatin quantum dots

Table 2 a

Mechanical properties of alginate-based active-intelligent films

Mechanical Properties Treatments

Thickness (mm) Control 0.006 ±0.001 A 0.0061±0.045 B 0.0059±0.071 C 0.006±0.053 D 0.0061±0.072

Tensile strength Control 14.86±0.87c A 52.7±1.93b B 52.7±2.07b C 62.8±1.41a D 62.8±1.82a

Elongation Control 29.4±2.57c A 30±1.06b B 30±1.3b C 35±1.11a D 35±1.04a

A, B, C, and D represent the films containing urea quantum dots, gelatin quantum dots, urea quantum                                        dots and mucilage, and gelatin quantum dots and mucilage. Data provided as mean ± standard deviation.                                      The significant difference is shown by superscript letters (P<0.05)

Table 2 b

Physical properties of alginate-based active-intelligent films

Physical Properties Treatments

Moisture content (%) Control 13.8±0.87a A 13.7±1.11a B 13.7±1.1a C 13.7±2.87a D 13.7±1.83a

Solubility (%) Control 93.6±2.57a A 65.2±1.32b B 65.2±1.32b C 60±4.24c D 60±5.04c

Water permeability (g/m-2 s-1) Control 2.6±0.17a A 1.3±0.41b B 1.3±0.7b C 1.1±0.49c D 1.1±0.47c

Contact angle ( ֯ ) Control 43.8±3.27c A 64.9±1.41b B 65±1.27b C 76.9±2.16a D 77±2.12a

A, B, C, and D represent the films containing urea quantum dots, gelatin quantum dots, urea quantum dots and mucilage, and gelatin quantum dots and mucilage. Data provided as mean ± standard deviation. The significant difference is shown by superscript letters (P<0.05)

Table 3

Transparency and opacity of alginate-based active-intelligent films

| Parameters |  |  | Treatments |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Control | A | B | C | D |
| Transparency Opacity | 99.2 0.74 | 82.9 17 | 81 18.9 | 74.8 25.1 | 73.2 26.7 |

A, B, C, and D represent the films containing urea quantum dots, gelatin quantum dots, urea quantum dots and mucilage, and gelatin quantum dots and mucilage

Table 4

Colorimetry of alginate-based active-intelligent films

| Treatments |  |  | Parameters |  |  |
| --- | --- | --- | --- | --- | --- |
|  | L* | a* | b* | ΔE | WI |
| Control A B C D | 88±3a 54.1±2.43b 54±1.17b 53.9±1.23b 54.2±1.56b | 1b 0c 0c 2a 2a | 1.9±0.7b 40±1a 41±0a 40±1a 41±0a | 10.9±1.43b 61±2.01a 61±2.03a 60.8±1.03a 60.7±0.03a | 89±1.43a 38.3±1.21b 37.9±0.12b 38±1.13b 38.1±1.41b |

A, B, C, and D represent the films containing urea quantum dots, gelatin quantum dots, urea quantum dots and mucilage, and gelatin quantum dots and mucilage. Data provided as mean ± standard deviation. The significant difference is shown by superscript letters (P<0.05)

Table 5

Microbial indices of quality in trout fillets during 16 days of filled storage (CFU/g-1)

Storage duration (day)

Parameters (bacteria) Treatments 0 4 8 12 16

Total Control 1±0.76 5±0.5 7.3±1 8.7±0 10.1±1 A 1±0.5 4±1 5±0 8.1±1 8.1±0 B 1±0.76 3.9±0.5 5±1 8.1±0 8.7±0 C 1±0.73 3.3±0.5 5.1±1 8.6±0 8.6±1 D 1±0.5 3.2±0.1 5.1±0 8±0.5 8.4±1

Psychrophilic Control 1±0.76 4±0.5 5±1 6.1±0 7.7±1 A 1±0.5 3±1 4.1±0 5.4±1 6±0 B 1±0.76 3±0.5 4±1 5.3±0 6.1±0 C 1±0.73 2.9±0.5 3.7±1 4.9±0 5.5±1 D 1±0.5 2.7±0.1 3.5±0 4.8±0.5 5.4±1

H2S-producing Control 1±0.76 3.8±0.5 5.6±1 6.8±0 7.6±1 A 1±0.5 2.9±1 5.3±0 5.8±1 7±0 B 1±0.76 2.7±0.5 4.4±1 5.7±0 7±0 C 1±0.73 2.6±0.5 5.3±1 5.6±0 7±1 D 1±0.5 2.4±0.1 4.4±0 5.3±0.5 7±1

A, B, C, and D represent the films containing urea quantum dots, gelatin quantum dots, urea quantum dots and mucilage, and gelatin quantum dots and mucilage. Data provided as mean ± standard deviation. The significant difference is shown by superscript letters (P<0.05)

Table 6

Chemical indices of quality in trout fillets during 16 days of filled storage

Storage duration (day)

Parameters Treatments 0 4 8 12 16

pH Control 5.6±0.08a 6.6±0.03a 8.1±0.009a 8.4±0.04a 8.8±0.04a A 5.6±0.08a 6.3±0.2b 7±0.04b 7.5±0.009c 8.5±0.04b B 5.6±0.08a 6.1±0.009c 6.6±0.06c 7.5±0.009c 8±0.04c C 5.6±0.08a 6±0.009c 6.2±0.01d 7.7±0.04b 7.8±0.09d D 5.6±0.08a 6.1±0.009c 6.3±0.05d 7.4±0.08c 7.7±0.09d

TVB-N Control 17.6±1.24b 35±2.94a 65.6±4.18a 88.3±1.69a 120.6±0.47a A 16.3±2.05b 23±1.41b 40.6±1.24b 65.6±0.47b 83±4.24b B 20.6±1.24b 24.6±3.77b 38.6±1.24b 63.3±3.09b 84.3±5.43b C 12.3±1.24c 20.3±1.24b 32.6±1.47c 59±1.63bc 76.6±0.94c D 14.6±0.94c 19.3±1.24b 32.6±1.69c 61.6±3.09c 76.3±0.47c

PV Control 0.11±0.008b 0.86±0.01a 5.5±0.03a 8.5±0.03a 12.8±0.02a A 0.11±0.008b 0.80±0.004b 3.4±0.01b 6.4±0.01b 8.3±0.005b B 0.14±0.02a 0.81±0.009b 3.6±0.009b 6.6±0.009b 7.9±0.68bc C 0.11±0.004b 0.77±0.01c 3.1±0.77c 4.8±1.23d 7.4±0.68c D 0.10±0.004b 0.77±0.008c 3.1±0.76c 5.7±1.22c 7.4±0.68c

TBA Control 0.05±0.004a 0.28±0.05a 0.5±0.008a 0.87±0.01a 1.07±0.01a A 0.05±0.004a 0.15±0.01b 0.3±0.02b 0.57±0.08b 1.02±0.001b B 0.05±0.004a 0.15±0.01b 0.3±0.01b 0.58±0.08b 1.02±0.004b C 0.05±0.004a 0.14±0.007b 0.3±0.01b 0.53±0.008c 0.97±0.1c D 0.05±0.004a 0.14±0.002b 0.2±0.01c 0.53±0.007c 0.94±0.06c

FFA Control 0.7±0a 0.92±0.04a 1.11±0.01a 1.3±0.02a 1.51±0.07a A 0.7±0a 0.87±0.004b 0.96±0.01b 1±0.01b 1.2±0.01b B 0.7±1.11a 0.86±0.009b 0.97±0.01b 1±0.01b 1.1±0.009b C 0.8±1.11a 0.88±0.009b 0.96±0.01c 1±0.01b 1.1±0.04c D 0.8±1.11a 0.88±0.004 0.98±0.02c 1±0.01b 1.1±0.004c

A, B, C, and D represent the films containing urea quantum dots, gelatin quantum dots, urea quantum dots and mucilage, and gelatin quantum dots and mucilage. TVB-N, PV, TBA, and FFA are respectively the abbreviations of Total volatile Basic Nitrogen, Peroxide Value, Thiobarbituric Acid, and Free Fatty Acids. Data provided as mean ± standard deviation. The significant difference is shown by superscript letters (P<0.05)

Table 7 A

The correlation between fluorescence and color changes with the level of bacteria in trout fillets

Treatments A B C D

Parameters R2 sig R2 sig R2 sig R2 sig

Total PL 0.848 0.01 0.952 0.002 0.973 0.01 0.995 0.02 ∆E 0.739 0.01 0.956 0.002 0.993 0.00 0.995 0.02

Psychrophilic PL 0.917 0.00 0.975 0.008 0.981 0.00 0.979 0.00 ∆E 0.817 0.03 0.935 0.01 0.991 0.01 0.969 0.01

H2S-producing PL 0.953 0.01 0.947 0.013 0.945 0.00 0.966 0.00 ∆E 0.821 0.01 0.934 0.022 0.945 0.00 0.956 0.01

A, B, C, and D represent the films containing urea quantum dots, gelatin quantum dots, urea quantum dots and mucilage, and gelatin quantum dots and mucilage

Table 7 B

The correlation between fluorescence and color changes with the level of pH and chemical compounds in trout fillets

Treatments A B C D

Parameters R2 sig R2 sig R2 sig R2 sig

pH PL 0.859 0.00 0.755 0.05 0.973 0.02 0.987 0.01 ∆E 0.793 0.01 0.871 0.01 0.961 0.00 0.983 0.01

TVB-N PL 0.738 0.00 0.863 0.001 0.959 0.01 0.994 0.03 ∆E 0.898 0.00 0.763 0.033 0.959 0.00 0.984 0.00

PV PL 0.855 0.01 0.955 0.01 0.933 0.01 0.957 0.00 ∆E 0.835 0.00 0.951 0.01 0.964 0.01 0.977 0.00

TBA PL 0.873 0.01 0.905 0.005 0.943 0.00 0.958 0.00 ∆E 0.895 0.01 0.92 0.013 0.971 0.00 0.98 0.00

FFA PL 0.839 0.03 0.855 0.00 0.833 0.00 0.875 0.00 ∆E 0.819 0.01 0.833 0.011 0.812 0.01 0.847 0.05

A, B, C, and D represent the films containing urea quantum dots, gelatin quantum dots, urea quantum dots and mucilage, and gelatin quantum dots and mucilage. TVB-N, PV, TBA, and FFA are respectively the abbreviations of Total volatile Basic Nitrogen, Peroxide Value, Thiobarbituric Acid, and Free Fatty Acids