Dimension compensation of desktop LCD 3D printer for high-precision microfluidic applications

Xinjie Zhang1,2*, Yuyang Liu1, Yang Bao1, Zixiao Zhen1, Jian Mi1, Yuxin Tang1, Qiwen Zhang3, Ayobami Elisha Oseyemi4

1College of Mechanical and Electrical Engineering, Hohai University, Changzhou 213200, China

2Department of Chemistry, School of Science, Tokyo Institute of Technology, Tokyo 152-8550, Japan

3Hohai-Lille College, Hohai University, Changzhou 213200, China

4Department of Mechanical Engineering, York University, Toronto ON M3J1P3, Canada

*Corresponding author: Xinjie Zhang (xj.zhang@hhu.edu.cn)

Tab. S1. Basic information of LCD 3D printer.

| Printer type | LCD X190 |
| --- | --- |
| Default printing accuracy (μm) | ± 50 |
| Screen resolution | 4 K (3840*2400) |
| Printing material | Photosensitive resin |
| Printer exterior dimension (mm) | 350*350*710 |
| Maximum printing size (mm) | 192*120*280 |
| Net weight (kg) | 25 |
| Exposure method | Strobe exposure and Constant exposure |

Tab. S2. Parameter settings of 3D printing.

| Bottom exposure time (s) | 15-25 |
| --- | --- |
| Normal layer exposure time (s) | 2-4 |
| Number of bottom layers | 30 |
| Number of transition layers | 40 |
| UV wavelength (nm) | 385 and 405 |
| Lifting distance (mm) | 12 |
| Bottom lifting distance (mm) | 10 |
| Return distance (mm) | 12 |
| Bottom return distance (mm) | 10 |
| Lifting speed (mm/min) | 300 |
| Bottom lifting Speed (mm/min) | 300 |
| Return speed (mm/min) | 300 |
| Bottom return speed (mm/min) | 300 |

Tab. S3. Physical property of liquid resin.

| Edition type | 150s |
| --- | --- |
| Appearance | Red wax |
| Proportion (25℃) | 1.05-1.13 |
| Viscosity | 350-550 cps |
| Critical exposure EC (mj/cm2) | 7 |
| Curing thickness Dp (mm) | 0.12 |

Tab. S4. Mechanical property of cured resin.

| Test items | Test methods | Numerical range |
| --- | --- | --- |
| Hardness (D) | ASTM D 2240 | 80 |
| Tensile strength (MPa) | ASTM D 638 | 32-37 |
| Break elongation (%) | ASTM D 638 | 4-7 |
| Glass transition temperature (℃) | ASTM D 648 | 65 |

Fig. S1. Pictures of post-treatment process for 3D-printed test molds.

Fig. S2. Pictures of PDMS demolding. (a) Mold without release agent. PDMS sheet was difficult to be peeled from the mold, resulting in a broken PDMS sheet. (b) Mold with release agent. After spraying release agent, PDMS sheet could be easily peeled from the mold. It is recommended to use the PDMS sheet after secondary demolding to obtain a high-quality microfluidic chip.

Fig. S3. PDMS chip bonding strength test. (a) Two PDMS chips prepared for bonding strength test in Z-axis and XY-plane directions. (b) Bonding strength test using a manual device with a push-pull force gauge. (c) Bonding strength test using an automated tensile testing device.

Fig. S4. Microfluidic chip bonding forces from (a) Z-axis and (b) XY-plane directions.

Fig. S5. Cross-sectional images of microchannels fabricated under the optimal layer thicknesses. Layer thickness of 35 µm was used for micro-scale and small-scale microchannel fabrication, while a layer thickness of 40 µm was used for tiny-scale microchannel fabrication. Scale bars 500 µm.

Fig. S6. Cross-sectional images of microchannels fabricated after dimension compensation. Scale bars 500 µm.

Fig. S7. Particle focusing and migration in the inertial microfluidic chip with trapezoidal-like cross-section. Flow rates of 1500-2600 µL/min and 2000-3000 µL/min were used for 15 µm and 10 µm particle experiments, respectively.