Supplementary Information

Wafer-scale monolayer organic single-crystalline films and arrays toward high-performance organic electronics

Ximeng Yao1,4, Chunli Ma1,4, Lingjie Sun2*, Xianshuo Wu1, Xianfeng Shen1, Zhaofeng Wang1, Shuyuan Yang1, Pichao Gao1, Dong Zeng1, Wei Deng3, Jiansheng Jie3, Fangxu Yang1, Rongjin Li1* and Wenping Hu1

1Key Laboratory of Organic Integrated Circuit, Ministry of Education & Tianjin Key Laboratory of Molecular Optoelectronic Sciences, Department of Chemistry, School of Science, Tianjin University, Tianjin 300072, China.

2Institute of Molecular Aggregation Science of Tianjin University, Tianjin 300072, China.

3Institute of Functional Nano & Soft Materials (FUNSOM), Jiangsu Key Laboratory for Carbon-Based Functional Materials & Devices Soochow University, Suzhou 215123, China.

4These authors contributed equally: Ximeng Yao, Chunli Ma.

*Correspondence to: lirj@tju.edu.cn; sunlingjie@tju.edu.cn

This PDF file includes:

Figs. S1 to S19

Table S1

Supplementary Figure 1 | Investigation into seed crystal adhesion with and without aging time. a Optical microscope (OM) images of PTS-modified Si/SiO2 substrates vertically immersed in top-phase solution after aging for 3 min, followed by rapid pulling. b OM image of a PTS-modified Si/SiO2 substrate vertically immersed in top-phase solution followed by rapid pulling in the absence of aging time.

Supplementary Figure 2 | OM images of 2DMCs by SDC at different withdrawal speed.

Supplementary Figure 3 | OM images of 2DMCs by SDC at different concentrations.

Supplementary Figure 4 | OM images of 2DMCs by SDC at different temperature.

Supplementary Figure 5 | Investigation into the Influence of different molar fractions of glycerol and water mixtures on the growth of 2DMCs by SDC.

Supplementary Figure 6 |OM images of 2DMCs by SDC at different solvent. The properties of the solvent are listed in the table S1 below. As the SDC growth of C10-DNTT 2DMCs occurs at elevated temperatures, selecting a solvent with a suitable boiling point is essential.

Supplementary Table 1 | Physical properties of different solvents used.

Supplementary Figure 7 | Investigation into the influence of upper solution volume of OSCs on the growth of 2DMCs by SDC.

Supplementary Figure 8 | OM images of 2DMCs by SDC with different aging times. a 0 min, b 3 min, and c 10 min

Supplementary Figure 9 | Random POM images of a wafer-scale monolayer C10-DNTT 2DMC acquired at a 3 × 3 matrix of positions.

Supplementary Figure 10 | Comparison of trap densities between C10-DNTT 2DMCs and other OSC single crystals. The data in Supplementary Fig. 10 are from refs35–40.

Supplementary Figure 11 | a Photograph of a wafer-scale, monolayer C6-DPA 2DMC film on a PTS-modified Si/SiO2 substrate. b POM images of a 3 x 3 matrix region across a wafer-scale, monolayer C6-DPA 2DMCs.

Supplementary Figure 12 | POM images of DTT-8, TFT-CN and Ph-BTBT-C10 2DMCs on PTS-modified Si/SiO2 substrate by SDC.

Supplementary Figure 13 | Out-of-plane XRD pattern of the DTT-8, TFT-CN and Ph-BTBT-C10 2DMCs.

Supplementary Figure 14 | Contact angle of substrates with different surface energies, and corresponding OM images of crystals prepared using the SDC method. a Contact angle of O2 plasma-modified Si/SiO2 substrate; b PTS-modified Si/SiO2 substrate; c OTS-modified Si/SiO2 substrate.d-f OM images of crystals prepared by the SDC method on the corresponding substrates.

Supplementary Figure 15 | Schematic illustration of the procedures to fabricate the wetting/dewetting patterns on the substrate.

Patterning of hydrophilic/hydrophobic regions enables spatial confinement of crystal growth on a substrate. This is achieved by using self-assembled monolayers (SAMs) of PTS/OTS as hydrophilic/hydrophobic materials (Supplementary Fig. 14 ). Initially, a desired pattern is deposited onto a hydrophilic substrate using shadow masks; here, we deposited metal thin films (10nm Au+100nm Cu) with triangular tip patterns to protect the underlying hydrophilic layer. Subsequently, the substrate surface is bombarded with oxygen plasma and then modified with an OTS hydrophobic layer. Afterward, a spin-coating PVA layer is used to lift off the metal pattern film. As a result, the desired PTS hydrophilic pattern is embedded within the hydrophobic OTS substrate (Supplementary Fig. 15).

Supplementary Figure 16 | The schematic step-by-step fabrication processes for the monolayer C10-DNTT 2DMC-based OFET array. The shape, spacing, and number of the electrode pairs are illustrative for better visibility.

Supplementary Figure 17 | Typical hysteresis curve of OFETs based on the C10-DNTT 2DMCs.

Supplementary Figure 18 | Transfer characteristics of 8×8 OFETs in the array. Channel length = 45 μm, and channel width = 80 μm.

Supplementary Figure 19 | Statistical data for the threshold voltage of the device array.