Additional file for “Evaluating the cradle-to-gate Environmental Impact and cooling performance of Advanced Daytime Radiative Cooling Materials to Establish a Comparative Framework for a Novel Photonic Meta-Concrete”

Adams, N.*1 , Carlosena, L.2 & Allacker, K.1

1KU Leuven, Faculty of Engineering Science, Department of Architecture, Kasteelpark Arenberg 1 – box 2431, 3001 Leuven, Belgium

2Engineering Department, Public University of Navarre (UPNA), Arrosadia Campus, 31006 Pamplona, Spain

(*) Corresponding author: Nick Adams: nick.adams@kuleuven.be

This Additional file contains the impact of the selected radiative cooling materials in the five selected impact categories (Figure S1-S8), the relationship between the cooling performance and the impact in the five selected impact categories (Figure S9-S13), the input data to model the selected radiative cooling materials using the Ecoinvent v3.6 database (Table S1), the emissivity of the selected radiative cooling materials in 39 wavebands (Table S2), the calculation of the sputter deposition parameters (Table S3), and the environmental impact of the ten selected radiative cooling materials in all impact categories (Table S4.1-S4.10).

| Figure S1. Particulate matter impact of the selected RC materials, showing the various components of the production process. | Figure S2. Particulate matter impact of the selected RC materials, showing the ratio of the various components in the production process. |
| --- | --- |

| Figure S3. Acidification impact of the selected RC materials, showing the various components of the production process. | Figure S4. Acidification impact of the selected RC materials, showing the ratio of the various components in the production process. |
| --- | --- |

| Figure S5. Resource use fossils impact of the selected RC materials, showing the various components of the production process. | Figure S6. Resource use fossils impact of the selected RC materials, showing the ratio of the various components in the production process. |
| --- | --- |

| Figure S7. Resource use minerals and metals impact of the selected RC materials, showing the various components of the production process. | Figure S8. Resource use minerals and metals impact the selected RC materials, showing the ratio of the various components in the production process. |
| --- | --- |

Figure S9. Relationship between accumulated radiated heat and solar gains (kWh·m-2) and global warming potential (kg CO2 eq.·dm-2), materials in the pareto front are highlighted with a border.

Figure S10. Relationship between accumulated radiated heat and solar gains (kWh·m-2) and particulate matter (disease inc.·dm-2), materials in the pareto front are highlighted with a border.

Figure S11. Relationship between accumulated radiated heat and solar gains (kWh·m-2) and acidification (mol H+ eq.·dm-2), materials in the pareto front are highlighted with a border.

Figure S12. Relationship between accumulated radiated heat and solar gains (kWh·m-2) and resource use fossils (MJ·dm-2), materials in the pareto front are highlighted with a border.

Figure S10. Relationship between accumulated radiated heat and solar gains (kWh·m-2) and resource use minerals and metals (kg Sb eq.·dm-2), materials in the pareto front are highlighted with a border.

Table S1. Input data to model the selected radiative cooling materials using the Ecoinvent v3.6 database.

| RC material | material/process | Ecoinvent v3.6 records | amount | unit | additional information |
| --- | --- | --- | --- | --- | --- |
| D1 | Titanium | Titanium, primary {GLO}¦ production ¦ Cut-off, U (RER electricity) | 0,00005771 | kg |  |
|  | Silicon | Silicon, solar grade {RER}¦ silicon production, solar grade, modified Siemens process ¦ Cut-off, U | 0,000014 | kg |  |
|  | silver | Silver {GLO}¦ market for ¦ Cut-off, U | 0,0000105 | kg |  |
|  | Si-wafer | Multi-Si wafer, ribbon {RER}¦ multi-Si wafer production, ribbon ¦ Cut-off, U | 0,01 | m2 |  |
|  | electricity | Electricity, medium voltage {RER}¦ market group for ¦ Cut-off, U | 6,42608101 | kWh |  |
|  | Argon gass | Argon, liquid {RER}¦ production ¦ Cut-off, U | 1341,14 | cm3 | input and emissions |
| D2 | Silicon | Silicon, solar grade {RER}¦ silicon production, solar grade, modified Siemens process ¦ Cut-off, U | 0,000308 | kg |  |
|  | Titanium | Titanium, primary {GLO}¦ production ¦ Cut-off, U (RER electricity) | 0,000316 | kg |  |
|  | Silver | Silver {GLO}¦ market for ¦ Cut-off, U | 0,000021 | kg |  |
|  | Si-wafer | Multi-Si wafer, ribbon {RER}¦ multi-Si wafer production, ribbon ¦ Cut-off, U | 0,01 | m2 |  |
|  | electricity | Electricity, medium voltage {RER}¦ market group for ¦ Cut-off, U | 34,3301478 | kWh |  |
|  | Argon gass | Argon, liquid {RER}¦ production ¦ Cut-off, U | 2513,02 | cm3 | input and emissions |
| D3 | Silicon | Silicon, solar grade {RER}¦ silicon production, solar grade, modified Siemens process ¦ Cut-off, U | 0,0001197 | kg |  |
|  | titanium | Titanium, primary {GLO}¦ production ¦ Cut-off, U (RER electricity) | 0,0000653 | kg |  |
|  | magnesiumsulfate | Magnesium sulfate {RER}¦ production ¦ Cut-off, U | 0,0001828 | kg |  |
|  | silver | Silver {GLO}¦ market for ¦ Cut-off, U | 0,0000105 | kg |  |
|  | Si-wafer | Multi-Si wafer, ribbon {RER}¦ multi-Si wafer production, ribbon ¦ Cut-off, U | 0,01 | m2 |  |
|  | electricity | Electricity, medium voltage {RER}¦ market group for ¦ Cut-off, U | 40,7826218 | kWh |  |
|  | Argon gass | Argon, liquid {RER}¦ production ¦ Cut-off, U | 2408,85 | cm3 | input and emissions |
|  | sheet rolling (only energy use) | Sheet rolling, aluminium {RER}¦ processing ¦ Cut-off, U | 0,0000598 | kg |  |
| D4 | 4-methyl-2-pentanone | 4-methyl-2-pentanone {RER}¦ production ¦ Cut-off, U | 0,00037694 | kg |  |
|  | silicon | Silicon, solar grade {RER}¦ silicon production, solar grade, modified Siemens process ¦ Cut-off, U | 0,0000699 | kg |  |
|  | silver | Silver {GLO}¦ market for ¦ Cut-off, U | 0,000042 | kg |  |
|  | sheet rolling (only energy use) | Sheet rolling, aluminium {RER}¦ processing ¦ Cut-off, U | 0,044684 | kg |  |
|  | Si-wafer | Multi-Si wafer, ribbon {RER}¦ multi-Si wafer production, ribbon ¦ Cut-off, U | 0,01 | m2 |  |
|  | electricity | Electricity, medium voltage {RER}¦ market group for ¦ Cut-off, U | 3,90700602 | kWh |  |
|  | Argon gass | Argon, liquid {RER}¦ production ¦ Cut-off, U | 260,41 | cm3 | input and emissions |
| D5 | silver | Silver {GLO}¦ market for ¦ Cut-off, U | 0,0000252 | kg |  |
|  | Polydimethylsiloxane | Polydimethylsiloxane {GLO}¦ polydimethylsiloxane production ¦ Cut-off, U | 0,00483 | kg |  |
|  | Si-wafer | Multi-Si wafer, ribbon {RER}¦ production ¦ Cut-off, U | 0,02 | m2 |  |
|  | extrusion (only energy use) | Extrusion, plastic film {RER}¦ extrusion, plastic film ¦ Cut-off, U | 0,00193 | kg |  |
|  | electricity | Electricity, medium voltage {RER}¦ market group for ¦ Cut-off, U | 3,66420361 | kWh |  |
|  | Argon gass | Argon, liquid {RER}¦ production ¦ Cut-off, U | 156,25 | cm3 | input and emissions |
| D6 | polystyrene | Polystyrene, general purpose {RER}¦ production ¦ Cut-off, U | 0,0003 | kg |  |
|  | steel | Reinforcing steel {RER}¦ production ¦ Cut-off, U | 0,0079 | kg |  |
|  | sheet rolling (only energy use) | Sheet rolling, steel {RER}¦ processing ¦ Cut-off, U | 0,0079 | kg |  |
|  | electricity | Electricity, medium voltage {RER}¦ market group for ¦ Cut-off, U | 0,0523 | kWh |  |
|  | Acetone | Acetone, liquid {RER}¦ production ¦ Cut-off, U | 0,0025 | kg | input and emissions |
|  | Nitrogen | Nitrogen, liquid {RER}¦ market for ¦ Cut-off, U | 0,0000021 | kg |  |
|  | water | Tap water {RER}¦ market group for ¦ Cut-off, U | 5 | l | input and emissions |
| D7 | polyvinylfluoride | Polyvinylfluoride {RoW}¦ production ¦ Cut-off, U | 0,0005 | kg |  |
|  | Aluminium | Aluminium, primary, ingot {IAI Area, EU27 & EFTA}¦ production ¦ Cut-off, U | 0,0054 | kg |  |
|  | sheet rolling (only energy use) | Sheet rolling, aluminium {RER}¦ processing ¦ Cut-off, U | 0,0054 | kg |  |
|  | electricity | Electricity, medium voltage {RER}¦ market group for ¦ Cut-off, U | 0,0523 | kWh |  |
|  | Acetone | Acetone, liquid {RER}¦ production ¦ Cut-off, U | 0,0025 | kg | input and emissions |
|  | Nitrogen | Nitrogen, liquid {RER}¦ market for ¦ Cut-off, U | 0,00000351 | kg |  |
|  | water | Tap water {RER}¦ market group for ¦ Cut-off, U | 5 | l | input and emissions |
| D8 | Silicon | Silicon, solar grade {RER}¦ silicon production, solar grade, modified Siemens process ¦ Cut-off, U | 0,000178 | kg |  |
|  | Si-wafer | Multi-Si wafer, ribbon {RER}¦ production ¦ Cut-off, U | 0,02 | m2 |  |
|  | electricity | Electricity, medium voltage {RER}¦ market group for ¦ Cut-off, U | 14,8725698 | kwh |  |
|  | Argon | Argon, liquid {RER}¦ production ¦ Cut-off, U | 7826,35468 | l | input and emissions |
| D9 | Silicon | Silicon, solar grade {RER}¦ silicon production, solar grade, modified Siemens process ¦ Cut-off, U | 0,00004862 | kg |  |
|  | titanium | Titanium, primary {GLO}¦ production ¦ Cut-off, U (RER electricity) | 0,00004199 | kg |  |
|  | silver | Silver {GLO}¦ market for ¦ Cut-off, U | 0,000042 | kg |  |
|  | Si-wafer | Multi-Si wafer, ribbon {RER}¦ production ¦ Cut-off, U | 0,01 | m2 |  |
|  | electricity | Electricity, medium voltage {RER}¦ market group for ¦ Cut-off, U | 8,69324849 | kwh |  |
|  | Argon | Argon, liquid {RER}¦ production ¦ Cut-off, U | 3647,37274 | l | input and emissions |
| D10 | Silicon | Silicon, solar grade {RER}¦ silicon production, solar grade, modified Siemens process ¦ Cut-off, U | 0,000142 | kg |  |
|  | titanium | Titanium, primary {GLO}¦ production ¦ Cut-off, U (RER electricity) | 0,000176 | kg |  |
|  | silver | Silver {GLO}¦ market for ¦ Cut-off, U | 0,000021 | kg |  |
|  | Si-wafer | Multi-Si wafer, ribbon {RER}¦ production ¦ Cut-off, U | 0,01 | m2 |  |
|  | electricity | Electricity, medium voltage {RER}¦ market group for ¦ Cut-off, U | 18,7877586 | kwh |  |
|  | Argon | Argon, liquid {RER}¦ production ¦ Cut-off, U | 10474,1379 | l | input and emissions |

Table S2. Emissivity of the selected daytime radiative cooling materials in the 39 wavebands used in the thermal radiation model for the ten selected radiative cooling materials and the concrete roof tile.

| Waveband | Emissivity |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | D1 | D2 | D3 | D4 | D5 | D6/D7 | D8 | D9 | D10 | Concrete roof tile |
| 1 | 0,345 | 0,080 | 0,570 | 0,840 | 0,875 | 0,024 | 0,440 | 0,370 | 0,032 | 0,642 |
| 2 | 0,454 | 0,086 | 0,570 | 0,501 | 0,518 | 0,021 | 0,045 | 0,371 | 0,006 | 0,642 |
| 3 | 0,239 | 0,024 | 0,239 | 0,034 | 0,023 | 0,021 | 0,026 | 0,031 | 0,005 | 0,594 |
| 4 | 0,036 | 0,019 | 0,067 | 0,026 | 0,023 | 0,029 | 0,005 | 0,023 | 0,022 | 0,599 |
| 5 | 0,074 | 0,077 | 0,030 | 0,041 | 0,047 | 0,060 | 0,233 | 0,013 | 0,007 | 0,647 |
| 6 | 0,047 | 0,005 | 0,040 | 0,098 | 0,129 | 0,225 | 0,582 | 0,013 | 0,031 | 0,850 |
| 7 | 0,003 | 0,016 | 0,101 | 0,519 | 0,188 | 0,405 | 0,785 | 0,226 | 0,058 | 0,921 |
| 8 | 0,017 | 0,057 | 0,162 | 0,742 | 0,668 | 0,479 | 0,698 | 0,225 | 0,018 | 0,928 |
| 9 | 0,085 | 0,058 | 0,103 | 0,404 | 0,465 | 0,383 | 0,854 | 0,020 | 0,014 | 0,926 |
| 10 | 0,106 | 0,062 | 0,169 | 0,373 | 0,532 | 0,450 | 0,957 | 0,016 | 0,019 | 0,928 |
| 11 | 0,047 | 0,062 | 0,077 | 0,386 | 0,825 | 0,497 | 0,879 | 0,018 | 0,135 | 0,929 |
| 12 | 0,021 | 0,087 | 0,390 | 0,678 | 0,948 | 0,730 | 0,903 | 0,082 | 0,108 | 0,933 |
| 13 | 0,030 | 0,154 | 0,078 | 0,947 | 0,951 | 0,978 | 0,813 | 0,136 | 0,489 | 0,888 |
| 14 | 0,158 | 0,580 | 0,457 | 0,873 | 0,952 | 0,977 | 0,968 | 0,377 | 0,962 | 0,923 |
| 15 | 0,428 | 0,923 | 0,787 | 0,913 | 0,983 | 0,966 | 0,704 | 0,726 | 0,837 | 0,938 |
| 16 | 0,494 | 0,719 | 0,667 | 0,933 | 0,985 | 0,973 | 0,633 | 0,744 | 0,798 | 0,943 |
| 17 | 0,682 | 0,629 | 0,520 | 0,951 | 0,941 | 0,972 | 0,699 | 0,811 | 0,860 | 0,945 |
| 18 | 0,864 | 0,687 | 0,631 | 0,954 | 0,889 | 0,977 | 0,749 | 0,871 | 0,898 | 0,943 |
| 19 | 0,969 | 0,763 | 0,851 | 0,948 | 0,897 | 0,964 | 0,793 | 0,750 | 0,599 | 0,937 |
| 20 | 0,599 | 0,795 | 0,686 | 0,956 | 0,901 | 0,941 | 0,802 | 0,627 | 0,611 | 0,918 |
| 21 | 0,203 | 0,762 | 0,684 | 0,912 | 0,935 | 0,922 | 0,860 | 0,655 | 0,722 | 0,913 |
| 22 | 0,170 | 0,864 | 0,631 | 0,931 | 0,969 | 0,946 | 0,896 | 0,520 | 0,783 | 0,915 |
| 23 | 0,177 | 0,957 | 0,684 | 0,955 | 0,955 | 0,947 | 0,883 | 0,520 | 0,832 | 0,922 |
| 24 | 0,172 | 0,955 | 0,790 | 0,935 | 0,906 | 0,947 | 0,880 | 0,561 | 0,884 | 0,923 |
| 25 | 0,160 | 0,963 | 0,798 | 0,883 | 0,899 | 0,949 | 0,893 | 0,502 | 0,919 | 0,925 |
| 26 | 0,151 | 0,961 | 0,609 | 0,865 | 0,930 | 0,956 | 0,903 | 0,445 | 0,923 | 0,928 |
| 27 | 0,154 | 0,959 | 0,730 | 0,850 | 0,941 | 0,949 | 0,924 | 0,427 | 0,903 | 0,928 |
| 28 | 0,174 | 0,972 | 0,528 | 0,848 | 0,952 | 0,973 | 0,904 | 0,362 | 0,606 | 0,931 |
| 29 | 0,170 | 0,960 | 0,248 | 0,898 | 0,960 | 0,989 | 0,877 | 0,341 | 0,447 | 0,900 |
| 30 | 0,170 | 0,960 | 0,393 | 0,927 | 0,965 | 0,990 | 0,862 | 0,346 | 0,421 | 0,900 |
| 31 | 0,170 | 0,960 | 0,536 | 0,889 | 0,965 | 0,995 | 0,844 | 0,339 | 0,316 | 0,900 |
| 32 | 0,170 | 0,960 | 0,826 | 0,907 | 0,955 | 0,990 | 0,853 | 0,325 | 0,351 | 0,900 |
| 33 | 0,170 | 0,960 | 0,748 | 0,959 | 0,977 | 0,990 | 0,936 | 0,317 | 0,265 | 0,900 |
| 34 | 0,170 | 0,960 | 0,701 | 0,933 | 0,952 | 0,990 | 0,668 | 0,328 | 0,257 | 0,900 |
| 35 | 0,170 | 0,960 | 0,628 | 0,924 | 0,943 | 0,990 | 0,668 | 0,370 | 0,227 | 0,900 |
| 36 | 0,170 | 0,960 | 0,684 | 0,944 | 0,983 | 0,990 | 0,728 | 0,427 | 0,288 | 0,900 |
| 37 | 0,170 | 0,960 | 0,791 | 0,877 | 0,967 | 0,990 | 0,764 | 0,400 | 0,546 | 0,900 |
| 38 | 0,170 | 0,960 | 0,682 | 0,850 | 0,950 | 0,990 | 0,760 | 0,400 | 0,500 | 0,900 |
| 39 | 0,170 | 0,960 | 0,650 | 0,850 | 0,950 | 0,990 | 0,760 | 0,400 | 0,000 | 0,900 |

Table S3. Calculation of the different sputter deposition parameters for the selected radiative cooling materials.

| Material | D1 | D2 | D3 | D4 | D5 | D6 | D7 | D8 | D9 | D10 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sputtering rate (nm/s) | 0,406 |  |  |  |  |  |  | 0,406 |  |  |
| sputter power (kW) | 0,436 |  |  |  |  |  |  | 0,436 |  |  |
| total sputter thickness (nm) | 1030,000 | 10224,000 | 12350,000 | 200,000 | 120,000 |  |  | 3813,000 | 1777,000 | 5103,000 |
| Sputter efficiency (%) | 50,000 |  |  |  |  |  |  |  |  |  |
| Sputter time (s) | 2536,946 | 25182,266 | 30418,719 | 492,611 | 295,567 |  |  | 9391,626 | 4376,847 | 12568,966 |
| target energy (kWh) | 0,307 | 3,050 | 3,684 | 0,060 | 0,036 |  |  | 1,137 | 0,530 | 1,522 |
| Argon rate (cc/min) | 50,000 |  |  |  |  |  |  |  |  |  |
| amount of argon (cc) | 2114,122 | 20985,222 | 25348,933 | 410,509 | 246,305 |  |  | 7826,355 | 3647,373 | 10474,138 |
| pumping time (s) | 2700,000 |  |  |  |  |  |  |  |  |  |
| total pumping time (s) | 5236,946 | 27882,266 | 33118,719 | 3192,611 | 2995,567 |  |  | 12091,626 | 7076,847 | 15268,966 |
| pumping power (kW) | 4,000 |  |  |  |  |  |  |  |  |  |
| Pumping energy (kWh) | 5,819 | 30,980 | 36,799 | 3,547 | 3,328 |  |  | 13,435 | 7,863 | 16,966 |
| cooling energy (kWh) | 0,300 |  |  |  |  |  |  |  |  |  |
| Total energy use (kWh) | 6,426 | 34,330 | 40,783 | 3,907 | 3,664 |  |  | 14,873 | 8,693 | 18,788 |

Table 4. Environmental impact of the ten selected radiative cooling materials using the impact categories of the EN15804+A2 standard.

Table S4.1. Radiative cooling material D1.

| Radiative cooling material D1 |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Impact Category | Unit | Total | Titanium | Silicon | Silicon | Titanium | Silver | Energy deposition | Silicon wafer | Argon | Energy cooling system | Energy pumps |
| Climate change | kg CO2 eq | 3,12E+00 | 1,12E-03 | 5,95E-04 | 7,93E-05 | 7,44E-05 | 4,96E-03 | 1,17E-01 | 6,93E-01 | 5,13E-03 | 7,67E-02 | 2,22E+00 |
| Ozone depletion | kg CFC11 eq | 5,70E-08 | 8,67E-11 | 2,27E-11 | 3,02E-12 | 5,78E-12 | 7,93E-11 | 1,92E-09 | 1,72E-08 | 8,84E-11 | 1,25E-09 | 3,63E-08 |
| Ionising radiation | kBq U-235 eq | 5,23E-01 | 1,09E-04 | 5,33E-05 | 7,10E-06 | 7,30E-06 | 2,11E-04 | 2,24E-02 | 6,11E-02 | 9,71E-04 | 1,46E-02 | 4,23E-01 |
| Photochemical ozone formation | kg NMVOC eq | 7,52E-03 | 4,35E-06 | 1,59E-06 | 2,13E-07 | 2,90E-07 | 4,85E-05 | 2,71E-04 | 1,87E-03 | 1,19E-05 | 1,77E-04 | 5,14E-03 |
| Particulate matter | disease inc. | 4,91E-08 | 5,56E-11 | 1,09E-11 | 1,46E-12 | 3,71E-12 | 3,55E-10 | 1,46E-09 | 1,86E-08 | 6,47E-11 | 9,56E-10 | 2,77E-08 |
| Human toxicity, non-cancer | CTUh | 2,98E-08 | 6,49E-11 | 7,12E-12 | 9,49E-13 | 4,33E-12 | 2,45E-10 | 1,05E-09 | 7,84E-09 | 4,63E-11 | 6,86E-10 | 1,98E-08 |
| Human toxicity, cancer | CTUh | 1,04E-09 | 5,12E-13 | 4,46E-13 | 5,95E-14 | 3,41E-14 | 5,82E-12 | 3,34E-11 | 3,44E-10 | 1,48E-12 | 2,19E-11 | 6,33E-10 |
| Acidification | mol H+ eq | 1,42E-02 | 5,70E-06 | 2,31E-06 | 3,08E-07 | 3,80E-07 | 5,61E-05 | 5,37E-04 | 3,02E-03 | 2,34E-05 | 3,51E-04 | 1,02E-02 |
| Eutrophication, freshwater | kg P eq | 2,61E-04 | 7,42E-08 | 2,97E-08 | 3,96E-09 | 4,95E-09 | 1,42E-06 | 1,04E-05 | 4,43E-05 | 4,54E-07 | 6,83E-06 | 1,98E-04 |
| Eutrophication, marine | kg N eq | 2,03E-03 | 8,94E-07 | 3,80E-07 | 5,07E-08 | 5,96E-08 | 1,61E-05 | 7,29E-05 | 5,05E-04 | 3,19E-06 | 4,77E-05 | 1,38E-03 |
| Eutrophication, terrestrial | mol N eq | 2,33E-02 | 9,99E-06 | 4,26E-06 | 5,69E-07 | 6,66E-07 | 2,05E-04 | 8,41E-04 | 5,71E-03 | 3,68E-05 | 5,50E-04 | 1,59E-02 |
| Ecotoxicity, freshwater | CTUe | 5,37E+00 | 5,25E-03 | 1,36E-03 | 1,81E-04 | 3,50E-04 | 2,51E-01 | 1,75E-01 | 1,49E+00 | 7,76E-03 | 1,15E-01 | 3,32E+00 |
| Land use | Pt | 1,02E+01 | 7,82E-03 | 2,34E-03 | 3,12E-04 | 5,21E-04 | 5,66E-02 | 3,70E-01 | 2,51E+00 | 1,62E-02 | 2,42E-01 | 7,01E+00 |
| Resource use, fossils | MJ | 6,15E+01 | 1,72E-02 | 9,43E-03 | 1,26E-03 | 1,15E-03 | 6,27E-02 | 2,46E+00 | 1,07E+01 | 1,08E-01 | 1,61E+00 | 4,66E+01 |
| Resource use, minerals and metals | kg Sb eq | 1,39E-05 | 4,02E-09 | 6,84E-10 | 9,12E-11 | 2,68E-10 | 8,27E-06 | 2,13E-07 | 1,26E-06 | 1,01E-08 | 1,39E-07 | 4,03E-06 |

Table S4.2. Radiative cooling material D2.

| Radiative cooling material D2 |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Impact Category | Unit | Total | Silicon | Titanium | Silver | Energy deposition | Argon | Silicon wafer | Energy cooling system | Energy pumps |
| Climate change | kg CO2 eq | 1,38E+01 | 1,31E-02 | 6,52E-03 | 9,93E-03 | 1,16E+00 | 5,09E-02 | 6,93E-01 | 7,67E-02 | 1,18E+01 |
| Ozone depletion | kg CFC11 eq | 2,33E-07 | 5,00E-10 | 5,07E-10 | 1,59E-10 | 1,90E-08 | 8,78E-10 | 1,72E-08 | 1,25E-09 | 1,93E-07 |
| Ionising radiation | kBq U-235 eq | 2,56E+00 | 1,17E-03 | 6,40E-04 | 4,23E-04 | 2,22E-01 | 9,64E-03 | 6,11E-02 | 1,46E-02 | 2,25E+00 |
| Photochemical ozone formation | kg NMVOC eq | 3,24E-02 | 3,51E-05 | 2,54E-05 | 9,70E-05 | 2,69E-03 | 1,18E-04 | 1,87E-03 | 1,77E-04 | 2,73E-02 |
| Particulate matter | disease inc. | 1,83E-07 | 2,41E-10 | 3,25E-10 | 7,11E-10 | 1,45E-08 | 6,42E-10 | 1,86E-08 | 9,56E-10 | 1,47E-07 |
| Human toxicity, non-cancer | CTUh | 1,26E-07 | 1,57E-10 | 3,79E-10 | 4,90E-10 | 1,04E-08 | 4,59E-10 | 7,84E-09 | 6,86E-10 | 1,06E-07 |
| Human toxicity, cancer | CTUh | 4,11E-09 | 9,83E-12 | 2,99E-12 | 1,16E-11 | 3,32E-10 | 1,47E-11 | 3,44E-10 | 2,19E-11 | 3,37E-09 |
| Acidification | mol H+ eq | 6,32E-02 | 5,09E-05 | 3,33E-05 | 1,12E-04 | 5,33E-03 | 2,33E-04 | 3,02E-03 | 3,51E-04 | 5,41E-02 |
| Eutrophication, freshwater | kg P eq | 1,22E-03 | 6,54E-07 | 4,34E-07 | 2,84E-06 | 1,04E-04 | 4,51E-06 | 4,43E-05 | 6,83E-06 | 1,05E-03 |
| Eutrophication, marine | kg N eq | 8,70E-03 | 8,38E-06 | 5,23E-06 | 3,22E-05 | 7,24E-04 | 3,16E-05 | 5,05E-04 | 4,77E-05 | 7,35E-03 |
| Eutrophication, terrestrial | mol N eq | 1,00E-01 | 9,40E-05 | 5,84E-05 | 4,11E-04 | 8,35E-03 | 3,65E-04 | 5,71E-03 | 5,50E-04 | 8,48E-02 |
| Ecotoxicity, freshwater | CTUe | 2,17E+01 | 2,99E-02 | 3,07E-02 | 5,02E-01 | 1,74E+00 | 7,71E-02 | 1,49E+00 | 1,15E-01 | 1,77E+01 |
| Land use | Pt | 4,41E+01 | 5,16E-02 | 4,57E-02 | 1,13E-01 | 3,68E+00 | 1,61E-01 | 2,51E+00 | 2,42E-01 | 3,73E+01 |
| Resource use, fossils | MJ | 2,86E+02 | 2,08E-01 | 1,00E-01 | 1,25E-01 | 2,44E+01 | 1,07E+00 | 1,07E+01 | 1,61E+00 | 2,48E+02 |
| Resource use, minerals and metals | kg Sb eq | 4,16E-05 | 1,51E-08 | 2,35E-08 | 1,65E-05 | 2,11E-06 | 1,00E-07 | 1,26E-06 | 1,39E-07 | 2,14E-05 |

Table S4.3. Radiative cooling material D3.

| Radiative cooling material D3 (part 1) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Impact Category | Unit | Total | Silicon | Silicon | Titanium | MagnesiumSulfate | Titanium | MagnesiumSulfate | Titanium | MagnesiumSulfate |
| Climate change | kg CO2 eq | 1,63E+01 | 9,41E-04 | 4,15E-03 | 2,33E-04 | 1,32E-06 | 4,65E-04 | 2,64E-06 | 6,51E-04 | 3,96E-06 |
| Ozone depletion | kg CFC11 eq | 2,73E-07 | 3,59E-11 | 1,58E-10 | 1,81E-11 | 2,11E-14 | 3,61E-11 | 4,22E-14 | 5,06E-11 | 6,32E-14 |
| Ionising radiation | kBq U-235 eq | 3,03E+00 | 8,43E-05 | 3,72E-04 | 2,28E-05 | 2,37E-07 | 4,56E-05 | 4,74E-07 | 6,39E-05 | 7,10E-07 |
| Photochemical ozone formation | kg NMVOC eq | 3,81E-02 | 2,52E-06 | 1,11E-05 | 9,05E-07 | 4,01E-09 | 1,81E-06 | 8,02E-09 | 2,53E-06 | 1,20E-08 |
| Particulate matter | disease inc. | 2,16E-07 | 1,73E-11 | 7,64E-11 | 1,16E-11 | 2,40E-13 | 2,32E-11 | 4,81E-13 | 3,24E-11 | 7,21E-13 |
| Human toxicity, non-cancer | CTUh | 1,48E-07 | 1,13E-11 | 4,97E-11 | 1,35E-11 | 1,24E-14 | 2,70E-11 | 2,47E-14 | 3,79E-11 | 3,71E-14 |
| Human toxicity, cancer | CTUh | 4,80E-09 | 7,06E-13 | 3,11E-12 | 1,07E-13 | 4,06E-16 | 2,13E-13 | 8,12E-16 | 2,99E-13 | 1,22E-15 |
| Acidification | mol H+ eq | 7,47E-02 | 3,66E-06 | 1,61E-05 | 1,19E-06 | 6,96E-09 | 2,38E-06 | 1,39E-08 | 3,33E-06 | 2,09E-08 |
| Eutrophication, freshwater | kg P eq | 1,43E-03 | 4,70E-08 | 2,07E-07 | 1,55E-08 | 1,13E-10 | 3,09E-08 | 2,26E-10 | 4,33E-08 | 3,39E-10 |
| Eutrophication, marine | kg N eq | 1,03E-02 | 6,02E-07 | 2,66E-06 | 1,86E-07 | 1,14E-09 | 3,73E-07 | 2,27E-09 | 5,22E-07 | 3,41E-09 |
| Eutrophication, terrestrial | mol N eq | 1,18E-01 | 6,75E-06 | 2,98E-05 | 2,08E-06 | 1,42E-08 | 4,16E-06 | 2,83E-08 | 5,83E-06 | 4,25E-08 |
| Ecotoxicity, freshwater | CTUe | 2,54E+01 | 2,15E-03 | 9,47E-03 | 1,09E-03 | 2,25E-06 | 2,19E-03 | 4,49E-06 | 3,06E-03 | 6,74E-06 |
| Land use | Pt | 5,19E+01 | 3,71E-03 | 1,63E-02 | 1,63E-03 | 4,39E-06 | 3,26E-03 | 8,77E-06 | 4,56E-03 | 1,32E-05 |
| Resource use, fossils | MJ | 3,38E+02 | 1,49E-02 | 6,59E-02 | 3,58E-03 | 2,68E-05 | 7,17E-03 | 5,36E-05 | 1,00E-02 | 8,04E-05 |
| Resource use, minerals and metals | kg Sb eq | 3,80E-05 | 1,08E-09 | 4,78E-09 | 8,39E-10 | 2,52E-12 | 1,68E-09 | 5,05E-12 | 2,35E-09 | 7,57E-12 |

| Radiative cooling material D3 (part 2) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Impact Category | Unit | Silver | Energy deposition | Argon | GlassSubstrate | Silicon wafer | Energy cooling system | Energy pumps | sheet rolling |
| Climate change | kg CO2 eq | 4,96E-03 | 1,41E+00 | 6,15E-02 | 3,16E-02 | 6,93E-01 | 7,67E-02 | 1,40E+01 | 3,06E-05 |
| Ozone depletion | kg CFC11 eq | 7,93E-11 | 2,30E-08 | 1,06E-09 | 6,82E-10 | 1,72E-08 | 1,25E-09 | 2,30E-07 | 6,15E-13 |
| Ionising radiation | kBq U-235 eq | 2,11E-04 | 2,68E-01 | 1,16E-02 | 3,73E-04 | 6,11E-02 | 1,46E-02 | 2,68E+00 | 2,47E-06 |
| Photochemical ozone formation | kg NMVOC eq | 4,85E-05 | 3,25E-03 | 1,42E-04 | 1,66E-04 | 1,87E-03 | 1,77E-04 | 3,25E-02 | 1,11E-07 |
| Particulate matter | disease inc. | 3,55E-10 | 1,75E-08 | 7,76E-10 | 3,11E-09 | 1,86E-08 | 9,56E-10 | 1,75E-07 | 9,90E-13 |
| Human toxicity, non-cancer | CTUh | 2,45E-10 | 1,26E-08 | 5,55E-10 | 2,28E-10 | 7,84E-09 | 6,86E-10 | 1,26E-07 | 4,01E-13 |
| Human toxicity, cancer | CTUh | 5,82E-12 | 4,01E-10 | 1,77E-11 | 6,48E-12 | 3,44E-10 | 2,19E-11 | 4,00E-09 | 1,90E-14 |
| Acidification | mol H+ eq | 5,61E-05 | 6,43E-03 | 2,81E-04 | 3,06E-04 | 3,02E-03 | 3,51E-04 | 6,43E-02 | 1,33E-07 |
| Eutrophication, freshwater | kg P eq | 1,42E-06 | 1,25E-04 | 5,45E-06 | 5,01E-07 | 4,43E-05 | 6,83E-06 | 1,25E-03 | 1,47E-09 |
| Eutrophication, marine | kg N eq | 1,61E-05 | 8,74E-04 | 3,82E-05 | 4,94E-05 | 5,05E-04 | 4,77E-05 | 8,73E-03 | 2,06E-08 |
| Eutrophication, terrestrial | mol N eq | 2,05E-04 | 1,01E-02 | 4,41E-04 | 6,03E-04 | 5,71E-03 | 5,50E-04 | 1,01E-01 | 2,30E-07 |
| Ecotoxicity, freshwater | CTUe | 2,51E-01 | 2,10E+00 | 9,31E-02 | 3,21E-01 | 1,49E+00 | 1,15E-01 | 2,10E+01 | 5,57E-05 |
| Land use | Pt | 5,66E-02 | 4,44E+00 | 1,94E-01 | 9,74E-02 | 2,51E+00 | 2,42E-01 | 4,44E+01 | 6,43E-05 |
| Resource use, fossils | MJ | 6,27E-02 | 2,95E+01 | 1,29E+00 | 3,25E-01 | 1,07E+01 | 1,61E+00 | 2,95E+02 | 4,68E-04 |
| Resource use, minerals and metals | kg Sb eq | 8,27E-06 | 2,55E-06 | 1,21E-07 | 1,76E-07 | 1,26E-06 | 1,39E-07 | 2,55E-05 | 5,81E-11 |

Table S4.4. Radiative cooling material D4.

| Radiative cooling material D4 |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Impact Category | Unit | Total | 4-methyl-2-pentanone | Sheet rolling | Silver | Silicon | Energy deposition | Argon | Silicon wafer | Energy cooling system | Energy pumps |
| Climate change | kg CO2 eq | 2,19E+00 | 1,02E-03 | 2,29E-02 | 1,99E-02 | 2,97E-03 | 2,28E-02 | 9,96E-04 | 6,93E-01 | 7,67E-02 | 1,35E+00 |
| Ozone depletion | kg CFC11 eq | 4,19E-08 | 1,47E-11 | 4,59E-10 | 3,17E-10 | 1,13E-10 | 3,73E-10 | 1,72E-11 | 1,72E-08 | 1,25E-09 | 2,21E-08 |
| Ionising radiation | kBq U-235 eq | 3,41E-01 | 3,43E-05 | 1,85E-03 | 8,46E-04 | 2,66E-04 | 4,34E-03 | 1,89E-04 | 6,11E-02 | 1,46E-02 | 2,58E-01 |
| Photochemical ozone formation | kg NMVOC eq | 5,53E-03 | 1,21E-05 | 8,28E-05 | 1,94E-04 | 7,97E-06 | 5,27E-05 | 2,31E-06 | 1,87E-03 | 1,77E-04 | 3,13E-03 |
| Particulate matter | disease inc. | 3,89E-08 | 3,44E-11 | 7,40E-10 | 1,42E-09 | 5,47E-11 | 2,84E-10 | 1,26E-11 | 1,86E-08 | 9,56E-10 | 1,69E-08 |
| Human toxicity, non-cancer | CTUh | 2,22E-08 | 1,44E-11 | 2,99E-10 | 9,79E-10 | 3,56E-11 | 2,03E-10 | 8,99E-12 | 7,84E-09 | 6,86E-10 | 1,21E-08 |
| Human toxicity, cancer | CTUh | 8,00E-10 | 1,62E-12 | 1,42E-11 | 2,33E-11 | 2,23E-12 | 6,49E-12 | 2,87E-13 | 3,44E-10 | 2,19E-11 | 3,86E-10 |
| Acidification | mol H+ eq | 1,00E-02 | 4,11E-06 | 9,94E-05 | 2,25E-04 | 1,16E-05 | 1,04E-04 | 4,55E-06 | 3,02E-03 | 3,51E-04 | 6,19E-03 |
| Eutrophication, freshwater | kg P eq | 1,81E-04 | 3,14E-08 | 1,10E-06 | 5,67E-06 | 1,48E-07 | 2,03E-06 | 8,82E-08 | 4,43E-05 | 6,83E-06 | 1,21E-04 |
| Eutrophication, marine | kg N eq | 1,49E-03 | 6,33E-07 | 1,54E-05 | 6,45E-05 | 1,90E-06 | 1,42E-05 | 6,19E-07 | 5,05E-04 | 4,77E-05 | 8,42E-04 |
| Eutrophication, terrestrial | mol N eq | 1,72E-02 | 7,15E-06 | 1,72E-04 | 8,21E-04 | 2,13E-05 | 1,63E-04 | 7,14E-06 | 5,71E-03 | 5,50E-04 | 9,71E-03 |
| Ecotoxicity, freshwater | CTUe | 4,72E+00 | 6,95E-03 | 4,16E-02 | 1,00E+00 | 6,78E-03 | 3,41E-02 | 1,51E-03 | 1,49E+00 | 1,15E-01 | 2,02E+00 |
| Land use | Pt | 7,40E+00 | 2,17E-03 | 4,80E-02 | 2,26E-01 | 1,17E-02 | 7,19E-02 | 3,14E-03 | 2,51E+00 | 2,42E-01 | 4,28E+00 |
| Resource use, fossils | MJ | 4,18E+01 | 2,37E-02 | 3,50E-01 | 2,51E-01 | 4,72E-02 | 4,78E-01 | 2,10E-02 | 1,07E+01 | 1,61E+00 | 2,84E+01 |
| Resource use, minerals and metals | kg Sb eq | 3,70E-05 | 6,90E-09 | 4,34E-08 | 3,31E-05 | 3,42E-09 | 4,13E-08 | 1,96E-09 | 1,26E-06 | 1,39E-07 | 2,46E-06 |

Table S4.5. Radiative cooling material D5.

| Radiative cooling material D5 |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Impact Category | Unit | Total | Silver | Polydimethylsiloxane | Silicon wafer | Energy deposition | Extrusion | Argon | Energy cooling system | Energy pumps | Energy spin coating |
| Climate change | kg CO2 eq | 2,84E+00 | 1,19E-02 | 8,21E-02 | 1,39E+00 | 1,37E-02 | 6,34E-04 | 5,97E-04 | 7,67E-02 | 1,27E+00 | 1,37E-03 |
| Ozone depletion | kg CFC11 eq | 5,60E-06 | 1,90E-10 | 5,54E-06 | 3,44E-08 | 2,24E-10 | 1,37E-11 | 1,03E-11 | 1,25E-09 | 2,08E-08 | 2,25E-11 |
| Ionising radiation | kBq U-235 eq | 3,84E-01 | 5,07E-04 | 1,70E-03 | 1,22E-01 | 2,61E-03 | 9,56E-05 | 1,13E-04 | 1,46E-02 | 2,42E-01 | 2,62E-04 |
| Photochemical ozone formation | kg NMVOC eq | 7,31E-03 | 1,16E-04 | 3,08E-04 | 3,73E-03 | 3,16E-05 | 1,90E-06 | 1,38E-06 | 1,77E-04 | 2,94E-03 | 3,18E-06 |
| Particulate matter | disease inc. | 6,02E-08 | 8,53E-10 | 5,27E-09 | 3,71E-08 | 1,70E-10 | 1,74E-11 | 7,54E-12 | 9,56E-10 | 1,58E-08 | 1,71E-11 |
| Human toxicity, non-cancer | CTUh | 3,03E-08 | 5,87E-10 | 1,83E-09 | 1,57E-08 | 1,22E-10 | 6,83E-12 | 5,39E-12 | 6,86E-10 | 1,14E-08 | 1,23E-11 |
| Human toxicity, cancer | CTUh | 1,15E-09 | 1,40E-11 | 6,14E-11 | 6,88E-10 | 3,89E-12 | 5,25E-13 | 1,72E-13 | 2,19E-11 | 3,62E-10 | 3,92E-13 |
| Acidification | mol H+ eq | 1,29E-02 | 1,35E-04 | 4,58E-04 | 6,04E-03 | 6,25E-05 | 3,09E-06 | 2,73E-06 | 3,51E-04 | 5,81E-03 | 6,29E-06 |
| Eutrophication, freshwater | kg P eq | 2,15E-04 | 3,40E-06 | 2,02E-06 | 8,85E-05 | 1,22E-06 | 5,28E-08 | 5,29E-08 | 6,83E-06 | 1,13E-04 | 1,22E-07 |
| Eutrophication, marine | kg N eq | 1,98E-03 | 3,87E-05 | 8,65E-05 | 1,01E-03 | 8,49E-06 | 4,97E-07 | 3,71E-07 | 4,77E-05 | 7,90E-04 | 8,54E-07 |
| Eutrophication, terrestrial | mol N eq | 2,27E-02 | 4,93E-04 | 9,57E-04 | 1,14E-02 | 9,80E-05 | 5,76E-06 | 4,28E-06 | 5,50E-04 | 9,11E-03 | 9,86E-06 |
| Ecotoxicity, freshwater | CTUe | 2,34E+01 | 6,02E-01 | 1,78E+01 | 2,98E+00 | 2,04E-02 | 1,72E-03 | 9,04E-04 | 1,15E-01 | 1,90E+00 | 2,05E-03 |
| Land use | Pt | 9,82E+00 | 1,36E-01 | 3,43E-01 | 5,03E+00 | 4,31E-02 | 1,23E-02 | 1,89E-03 | 2,42E-01 | 4,01E+00 | 4,34E-03 |
| Resource use, fossils | MJ | 5,10E+01 | 1,50E-01 | 9,22E-01 | 2,13E+01 | 2,87E-01 | 1,32E-02 | 1,26E-02 | 1,61E+00 | 2,67E+01 | 2,88E-02 |
| Resource use, minerals and metals | kg Sb eq | 2,52E-05 | 1,98E-05 | 3,56E-07 | 2,52E-06 | 2,48E-08 | 1,73E-09 | 1,17E-09 | 1,39E-07 | 2,30E-06 | 2,49E-09 |

Table S4.6. Radiative cooling material D6.

| Radiative cooling material D6 |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Impact Category | Unit | Total | Polystyrene | Steel | Sheet rolling | Energy | water | Acetone | nitrogen |
| Climate change | kg CO2 eq | 4,88E-02 | 1,17E-03 | 1,74E-02 | 2,58E-03 | 2,00E-02 | 1,64E-03 | 6,09E-03 | 4,61E-07 |
| Ozone depletion | kg CFC11 eq | 7,72E-10 | 5,14E-13 | 3,39E-10 | 6,11E-11 | 3,27E-10 | 4,33E-11 | 1,78E-12 | 7,59E-15 |
| Ionising radiation | kBq U-235 eq | 4,36E-03 | 5,48E-08 | 2,24E-04 | 1,41E-04 | 3,81E-03 | 1,87E-04 | 2,58E-07 | 8,63E-08 |
| Photochemical ozone formation | kg NMVOC eq | 1,71E-04 | 2,89E-06 | 8,23E-05 | 1,11E-05 | 4,62E-05 | 5,74E-06 | 2,24E-05 | 1,12E-09 |
| Particulate matter | disease inc. | 1,96E-09 | 3,65E-11 | 1,24E-09 | 1,15E-10 | 2,49E-10 | 7,71E-11 | 2,44E-10 | 6,39E-15 |
| Human toxicity, non-cancer | CTUh | 8,50E-10 | 2,57E-12 | 5,08E-10 | 3,98E-11 | 1,78E-10 | 9,80E-11 | 1,24E-11 | 4,21E-15 |
| Human toxicity, cancer | CTUh | 1,33E-10 | 1,18E-13 | 1,08E-10 | 1,12E-11 | 5,69E-12 | 6,77E-12 | 5,80E-13 | 1,37E-16 |
| Acidification | mol H+ eq | 2,12E-04 | 4,07E-06 | 6,71E-05 | 1,03E-05 | 9,13E-05 | 8,39E-06 | 3,11E-05 | 2,12E-09 |
| Eutrophication, freshwater | kg P eq | 3,19E-06 | 9,90E-10 | 8,45E-07 | 1,21E-07 | 1,78E-06 | 1,11E-07 | 3,36E-07 | 4,04E-11 |
| Eutrophication, marine | kg N eq | 3,57E-05 | 6,32E-07 | 1,47E-05 | 2,09E-06 | 1,24E-05 | 1,39E-06 | 4,49E-06 | 3,01E-10 |
| Eutrophication, terrestrial | mol N eq | 4,03E-04 | 6,84E-06 | 1,64E-04 | 2,36E-05 | 1,43E-04 | 1,57E-05 | 4,91E-05 | 3,46E-09 |
| Ecotoxicity, freshwater | CTUe | 1,64E-01 | 2,67E-04 | 1,08E-01 | 7,69E-03 | 2,99E-02 | 6,17E-03 | 4,66E-03 | 7,45E-07 |
| Land use | Pt | 1,24E-01 | 1,66E-05 | 4,74E-02 | 7,63E-03 | 6,30E-02 | 6,01E-03 | 6,56E-05 | 1,53E-06 |
| Resource use, fossils | MJ | 8,41E-01 | 2,44E-02 | 1,80E-01 | 3,61E-02 | 4,19E-01 | 2,76E-02 | 1,55E-01 | 9,61E-06 |
| Resource use, minerals and metals | kg Sb eq | 1,02E-07 | 1,23E-10 | 5,22E-08 | 3,73E-09 | 3,62E-08 | 8,06E-09 | 1,24E-09 | 9,12E-13 |

Table S4.7. Radiative cooling material D7.

| Radiative cooling material D7 |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Impact Category | Unit | Total | Polyvinylfluoride | Aluminium | Sheet rolling | Energy | water | Acetone | nitrogen |
| Climate change | kg CO2 eq | 7,93E-02 | 8,35E-03 | 4,05E-02 | 2,76E-03 | 2,00E-02 | 1,64E-03 | 6,09E-03 | 7,71E-07 |
| Ozone depletion | kg CFC11 eq | 1,64E-09 | 7,61E-11 | 1,14E-09 | 5,55E-11 | 3,27E-10 | 4,33E-11 | 1,78E-12 | 1,27E-14 |
| Ionising radiation | kBq U-235 eq | 7,80E-03 | 1,97E-04 | 3,38E-03 | 2,23E-04 | 3,81E-03 | 1,87E-04 | 2,58E-07 | 1,44E-07 |
| Photochemical ozone formation | kg NMVOC eq | 2,37E-04 | 1,81E-05 | 1,34E-04 | 1,00E-05 | 4,62E-05 | 5,74E-06 | 2,24E-05 | 1,87E-09 |
| Particulate matter | disease inc. | 3,46E-09 | 2,58E-10 | 2,55E-09 | 8,94E-11 | 2,49E-10 | 7,71E-11 | 2,44E-10 | 1,07E-14 |
| Human toxicity, non-cancer | CTUh | 2,12E-09 | 1,04E-10 | 1,68E-09 | 3,62E-11 | 1,78E-10 | 9,80E-11 | 1,24E-11 | 7,03E-15 |
| Human toxicity, cancer | CTUh | 1,38E-10 | 2,26E-12 | 1,21E-10 | 1,71E-12 | 5,69E-12 | 6,77E-12 | 5,80E-13 | 2,29E-16 |
| Acidification | mol H+ eq | 4,21E-04 | 3,47E-05 | 2,43E-04 | 1,20E-05 | 9,13E-05 | 8,39E-06 | 3,11E-05 | 3,55E-09 |
| Eutrophication, freshwater | kg P eq | 4,62E-06 | 2,23E-07 | 2,04E-06 | 1,33E-07 | 1,78E-06 | 1,11E-07 | 3,36E-07 | 6,75E-11 |
| Eutrophication, marine | kg N eq | 5,31E-05 | 4,77E-06 | 2,82E-05 | 1,86E-06 | 1,24E-05 | 1,39E-06 | 4,49E-06 | 5,04E-10 |
| Eutrophication, terrestrial | mol N eq | 5,91E-04 | 5,35E-05 | 3,09E-04 | 2,08E-05 | 1,43E-04 | 1,57E-05 | 4,91E-05 | 5,79E-09 |
| Ecotoxicity, freshwater | CTUe | 1,86E-01 | 1,65E-02 | 1,17E-01 | 5,03E-03 | 2,99E-02 | 6,17E-03 | 4,66E-03 | 1,25E-06 |
| Land use | Pt | 1,29E-01 | 1,29E-02 | 4,10E-02 | 5,80E-03 | 6,30E-02 | 6,01E-03 | 6,56E-05 | 2,56E-06 |
| Resource use, fossils | MJ | 1,29E+00 | 7,30E-02 | 5,78E-01 | 4,23E-02 | 4,19E-01 | 2,76E-02 | 1,55E-01 | 1,61E-05 |
| Resource use, minerals and metals | kg Sb eq | 1,92E-07 | 7,77E-08 | 6,39E-08 | 5,25E-09 | 3,62E-08 | 8,06E-09 | 1,24E-09 | 1,52E-12 |

Table S4.8. Radiative cooling material D8.

| Radiative cooling material D8 |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Impact Category | Unit | Total | Argon | Energy deposition | Energy pumps | Energy cooling system | Silicon | Silicon wafer |
| Climate change | kg CO2 eq | 6,36E+00 | 1,90E-02 | 4,34E-01 | 5,13E+00 | 7,67E-02 | 7,56E-03 | 6,93E-01 |
| Ozone depletion | kg CFC11 eq | 1,10E-07 | 3,27E-10 | 7,10E-09 | 8,39E-08 | 1,25E-09 | 2,88E-10 | 1,72E-08 |
| Ionising radiation | kBq U-235 eq | 1,14E+00 | 3,60E-03 | 8,28E-02 | 9,78E-01 | 1,46E-02 | 6,77E-04 | 6,11E-02 |
| Photochemical ozone formation | kg NMVOC eq | 1,50E-02 | 4,40E-05 | 1,00E-03 | 1,19E-02 | 1,77E-04 | 2,03E-05 | 1,87E-03 |
| Particulate matter | disease inc. | 8,92E-08 | 2,39E-10 | 5,41E-09 | 6,39E-08 | 9,56E-10 | 1,39E-10 | 1,86E-08 |
| Human toxicity, non-cancer | CTUh | 5,85E-08 | 1,71E-10 | 3,88E-09 | 4,58E-08 | 6,86E-10 | 9,04E-11 | 7,84E-09 |
| Human toxicity, cancer | CTUh | 1,96E-09 | 5,47E-12 | 1,24E-10 | 1,46E-09 | 2,19E-11 | 5,67E-12 | 3,44E-10 |
| Acidification | mol H+ eq | 2,89E-02 | 8,68E-05 | 1,99E-03 | 2,35E-02 | 3,51E-04 | 2,93E-05 | 3,02E-03 |
| Eutrophication, freshwater | kg P eq | 5,48E-04 | 1,68E-06 | 3,87E-05 | 4,57E-04 | 6,83E-06 | 3,77E-07 | 4,43E-05 |
| Eutrophication, marine | kg N eq | 4,03E-03 | 1,18E-05 | 2,70E-04 | 3,19E-03 | 4,77E-05 | 4,83E-06 | 5,05E-04 |
| Eutrophication, terrestrial | mol N eq | 4,64E-02 | 1,36E-04 | 3,11E-03 | 3,68E-02 | 5,50E-04 | 5,42E-05 | 5,71E-03 |
| Ecotoxicity, freshwater | CTUe | 9,97E+00 | 2,87E-02 | 6,49E-01 | 7,67E+00 | 1,15E-01 | 1,72E-02 | 1,49E+00 |
| Land use | Pt | 2,04E+01 | 5,99E-02 | 1,37E+00 | 1,62E+01 | 2,42E-01 | 2,97E-02 | 2,51E+00 |
| Resource use, fossils | MJ | 1,29E+02 | 4,00E-01 | 9,11E+00 | 1,08E+02 | 1,61E+00 | 1,20E-01 | 1,07E+01 |
| Resource use, minerals and metals | kg Sb eq | 1,15E-05 | 3,73E-08 | 7,87E-07 | 9,30E-06 | 1,39E-07 | 8,69E-09 | 1,26E-06 |

Table S4.9. Radiative cooling material D9.

| Radiative cooling material D9 (Part 1) |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Impact Category | Unit | Total | Silicon | Titanium | Silicon | Titanium | Silicon | Titanium | Silicon | Silver |
| Climate change | kg CO2 eq | 4,03E+00 | 4,56E-04 | 9,02E-04 | 1,36E-03 | 2,42E-05 | 1,45E-04 | 6,32E-05 | 1,07E-04 | 1,99E-02 |
| Ozone depletion | kg CFC11 eq | 7,19E-08 | 1,74E-11 | 7,01E-11 | 5,20E-11 | 1,88E-12 | 5,52E-12 | 4,91E-12 | 4,08E-12 | 3,17E-10 |
| Ionising radiation | kBq U-235 eq | 6,94E-01 | 4,08E-05 | 8,85E-05 | 1,22E-04 | 2,37E-06 | 1,30E-05 | 6,20E-06 | 9,59E-06 | 8,46E-04 |
| Photochemical ozone formation | kg NMVOC eq | 9,73E-03 | 1,22E-06 | 3,51E-06 | 3,66E-06 | 9,41E-08 | 3,88E-07 | 2,46E-07 | 2,87E-07 | 1,94E-04 |
| Particulate matter | disease inc. | 6,13E-08 | 8,39E-12 | 4,49E-11 | 2,51E-11 | 1,20E-12 | 2,66E-12 | 3,15E-12 | 1,97E-12 | 1,42E-09 |
| Human toxicity, non-cancer | CTUh | 3,85E-08 | 5,46E-12 | 5,25E-11 | 1,63E-11 | 1,41E-12 | 1,73E-12 | 3,68E-12 | 1,28E-12 | 9,79E-10 |
| Human toxicity, cancer | CTUh | 1,31E-09 | 3,42E-13 | 4,14E-13 | 1,02E-12 | 1,11E-14 | 1,08E-13 | 2,90E-14 | 8,03E-14 | 2,33E-11 |
| Acidification | mol H+ eq | 1,84E-02 | 1,77E-06 | 4,61E-06 | 5,29E-06 | 1,24E-07 | 5,62E-07 | 3,23E-07 | 4,16E-07 | 2,25E-04 |
| Eutrophication, freshwater | kg P eq | 3,45E-04 | 2,28E-08 | 6,00E-08 | 6,81E-08 | 1,61E-09 | 7,22E-09 | 4,20E-09 | 5,34E-09 | 5,67E-06 |
| Eutrophication, marine | kg N eq | 2,63E-03 | 2,92E-07 | 7,23E-07 | 8,72E-07 | 1,94E-08 | 9,26E-08 | 5,07E-08 | 6,85E-08 | 6,45E-05 |
| Eutrophication, terrestrial | mol N eq | 3,03E-02 | 3,27E-06 | 8,08E-06 | 9,78E-06 | 2,16E-07 | 1,04E-06 | 5,66E-07 | 7,68E-07 | 8,21E-04 |
| Ecotoxicity, freshwater | CTUe | 7,46E+00 | 1,04E-03 | 4,24E-03 | 3,11E-03 | 1,14E-04 | 3,30E-04 | 2,97E-04 | 2,44E-04 | 1,00E+00 |
| Land use | Pt | 1,32E+01 | 1,79E-03 | 6,32E-03 | 5,37E-03 | 1,69E-04 | 5,70E-04 | 4,43E-04 | 4,21E-04 | 2,26E-01 |
| Resource use, fossils | MJ | 8,05E+01 | 7,23E-03 | 1,39E-02 | 2,16E-02 | 3,73E-04 | 2,30E-03 | 9,74E-04 | 1,70E-03 | 2,51E-01 |
| Resource use, minerals and metals | kg Sb eq | 4,03E-05 | 5,24E-10 | 3,25E-09 | 1,57E-09 | 8,72E-11 | 1,66E-10 | 2,28E-10 | 1,23E-10 | 3,31E-05 |

| Radiative cooling material D9 (Part 2) |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Impact Category | Unit | Titanium | Energy deposition | Argon | Silicon wafer | Energy cooling system | Energy pumps |
| Climate change | kg CO2 eq | 6,31E-05 | 2,05E-01 | 8,95E-03 | 6,93E-01 | 7,67E-02 | 3,02E+00 |
| Ozone depletion | kg CFC11 eq | 4,90E-12 | 3,35E-09 | 1,54E-10 | 1,72E-08 | 1,25E-09 | 4,94E-08 |
| Ionising radiation | kBq U-235 eq | 6,20E-06 | 3,90E-02 | 1,69E-03 | 6,11E-02 | 1,46E-02 | 5,76E-01 |
| Photochemical ozone formation | kg NMVOC eq | 2,46E-07 | 4,73E-04 | 2,07E-05 | 1,87E-03 | 1,77E-04 | 6,99E-03 |
| Particulate matter | disease inc. | 3,14E-12 | 2,55E-09 | 1,13E-10 | 1,86E-08 | 9,56E-10 | 3,76E-08 |
| Human toxicity, non-cancer | CTUh | 3,67E-12 | 1,83E-09 | 8,07E-11 | 7,84E-09 | 6,86E-10 | 2,70E-08 |
| Human toxicity, cancer | CTUh | 2,90E-14 | 5,83E-11 | 2,58E-12 | 3,44E-10 | 2,19E-11 | 8,61E-10 |
| Acidification | mol H+ eq | 3,23E-07 | 9,36E-04 | 4,09E-05 | 3,02E-03 | 3,51E-04 | 1,38E-02 |
| Eutrophication, freshwater | kg P eq | 4,20E-09 | 1,82E-05 | 7,92E-07 | 4,43E-05 | 6,83E-06 | 2,69E-04 |
| Eutrophication, marine | kg N eq | 5,06E-08 | 1,27E-04 | 5,56E-06 | 5,05E-04 | 4,77E-05 | 1,88E-03 |
| Eutrophication, terrestrial | mol N eq | 5,65E-07 | 1,47E-03 | 6,42E-05 | 5,71E-03 | 5,50E-04 | 2,17E-02 |
| Ecotoxicity, freshwater | CTUe | 2,97E-04 | 3,06E-01 | 1,35E-02 | 1,49E+00 | 1,15E-01 | 4,52E+00 |
| Land use | Pt | 4,42E-04 | 6,46E-01 | 2,83E-02 | 2,51E+00 | 2,42E-01 | 9,54E+00 |
| Resource use, fossils | MJ | 9,73E-04 | 4,29E+00 | 1,88E-01 | 1,07E+01 | 1,61E+00 | 6,34E+01 |
| Resource use, minerals and metals | kg Sb eq | 2,28E-10 | 3,71E-07 | 1,76E-08 | 1,26E-06 | 1,39E-07 | 5,48E-06 |

Table S4.10. Radiative cooling material D10.

| Radiative cooling material D10 |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Impact Category | Unit | Total | Silicon | Titanium | Silver | Energy deposition | Argon | Silicon wafer | Energy cooling system | Energy pumps |
| Climate change | kg CO2 eq | 7,87E+00 | 6,03E-03 | 3,64E-03 | 9,93E-03 | 5,81E-01 | 2,54E-02 | 6,93E-01 | 7,67E-02 | 6,47E+00 |
| Ozone depletion | kg CFC11 eq | 1,35E-07 | 2,30E-10 | 2,83E-10 | 1,59E-10 | 9,50E-09 | 4,38E-10 | 1,72E-08 | 1,25E-09 | 1,06E-07 |
| Ionising radiation | kBq U-235 eq | 1,43E+00 | 5,41E-04 | 3,57E-04 | 4,23E-04 | 1,11E-01 | 4,81E-03 | 6,11E-02 | 1,46E-02 | 1,23E+00 |
| Photochemical ozone formation | kg NMVOC eq | 1,85E-02 | 1,62E-05 | 1,42E-05 | 9,70E-05 | 1,34E-03 | 5,89E-05 | 1,87E-03 | 1,77E-04 | 1,50E-02 |
| Particulate matter | disease inc. | 1,09E-07 | 1,11E-10 | 1,81E-10 | 7,11E-10 | 7,24E-09 | 3,20E-10 | 1,86E-08 | 9,56E-10 | 8,07E-08 |
| Human toxicity, non-cancer | CTUh | 7,26E-08 | 7,22E-11 | 2,12E-10 | 4,90E-10 | 5,19E-09 | 2,29E-10 | 7,84E-09 | 6,86E-10 | 5,79E-08 |
| Human toxicity, cancer | CTUh | 2,40E-09 | 4,52E-12 | 1,67E-12 | 1,16E-11 | 1,66E-10 | 7,33E-12 | 3,44E-10 | 2,19E-11 | 1,85E-09 |
| Acidification | mol H+ eq | 3,59E-02 | 2,34E-05 | 1,86E-05 | 1,12E-04 | 2,66E-03 | 1,16E-04 | 3,02E-03 | 3,51E-04 | 2,96E-02 |
| Eutrophication, freshwater | kg P eq | 6,85E-04 | 3,01E-07 | 2,42E-07 | 2,84E-06 | 5,17E-05 | 2,25E-06 | 4,43E-05 | 6,83E-06 | 5,77E-04 |
| Eutrophication, marine | kg N eq | 4,99E-03 | 3,86E-06 | 2,92E-06 | 3,22E-05 | 3,61E-04 | 1,58E-05 | 5,05E-04 | 4,77E-05 | 4,02E-03 |
| Eutrophication, terrestrial | mol N eq | 5,76E-02 | 4,33E-05 | 3,26E-05 | 4,11E-04 | 4,17E-03 | 1,82E-04 | 5,71E-03 | 5,50E-04 | 4,65E-02 |
| Ecotoxicity, freshwater | CTUe | 1,27E+01 | 1,38E-02 | 1,71E-02 | 5,02E-01 | 8,69E-01 | 3,85E-02 | 1,49E+00 | 1,15E-01 | 9,68E+00 |
| Land use | Pt | 2,53E+01 | 2,38E-02 | 2,55E-02 | 1,13E-01 | 1,83E+00 | 8,02E-02 | 2,51E+00 | 2,42E-01 | 2,04E+01 |
| Resource use, fossils | MJ | 1,61E+02 | 9,57E-02 | 5,61E-02 | 1,25E-01 | 1,22E+01 | 5,35E-01 | 1,07E+01 | 1,61E+00 | 1,36E+02 |
| Resource use, minerals and metals | kg Sb eq | 3,08E-05 | 6,94E-09 | 1,31E-08 | 1,65E-05 | 1,05E-06 | 4,99E-08 | 1,26E-06 | 1,39E-07 | 1,17E-05 |