Support material

A novel photothermal energy storage phase change material with high stability and enthalpy

Shenghua Xiong a,b, Yanlong Shi a,b Changhui Liu a,b, Gang Lia,b*, and Yunyun Yang a,b*

a: College of Civil Aviation Safety Engineering, Civil Aviation Flight University of China, Guanghan 618307, China
b: Civil Aircraft Fire Science and Safety Engineering Key Laboratory of Sichuan Province, Civil Aviation Flight University of China, Guanghan 618307, China

*: Corresponding authors: yunyun1990@cafuc.edu.cn, ligang@cafuc.edu.cn

Table S1. The related TGA and DTG data of CNT-SA, CNT-BN-SA-1 and CNT-BN-SA-2.

| Samples | T5%(℃)a | T50%(℃)b | TP(℃)c | PL(%/min)d |
| --- | --- | --- | --- | --- |
| CNT-SA | 200.5 | 248.0 | 255.5 | -18.2 |
| CNT-BN-SA-1 | 205.5 | 258.0 | 258.0 | -14.1 |
| CNT-BN-SA-2 | 193.1 | 245.6 | 250.1 | -18.8 |

a: The testing temperature when the mass-loss of sample reaches 5wt.%

b: The testing temperature when the mass-loss of sample reaches 50wt.%

c: The testing temperature of mass-loss peak

d: The mass-loss rate of the mass-loss peak

Table S2. The phase-change properties of CNT-SA, CNT-BN-SA-1, CNT-BN-SA-2, and CNT-SA-1k, CNT-BN-SA-1-1k, CNT-BN-SA-2-1k

| Samples | Tc(℃)a | Tm(℃)b | △Hc (J/g)c |  | △Hm (J/g)d |
| --- | --- | --- | --- | --- | --- |
| SA | 52.23 | 51.5 |  | 189.4 | 178.9 |
| CNT-SA | 51.96 | 50.81 |  | 141.2 | 135.0 |
| CNT-BN-SA-1 | 52.66 | 51.83 |  | 150.4 | 143.5 |
| CNT-BN-SA-2 | 52.67 | 51.2 |  | 139.5 | 131.6 |
| CNT-SA-1k | 51.9 | 50.79 |  | 136.4 | 132.6 |
| CNT-BN-SA-1-1k | 52.86 | 51.53 |  | 147.5 | 147.3 |
| CNT-BN-SA-2-1k | 52.75 | 51.00 |  | 146.7 | 138.3 |

a: The crystalline temperature during cooling

b: The melting temperature during heating

c: The crystalline enthalpy during cooling

d: The melting enthalpy during heating

Figure S1. The DSC curves of SA.