Supplementary Information for

Ultrathin Glass-based Perovskite Solar Cells Employing Bilayer Electron Transport Layer

Wooyeon Kim1,‡, Jian Cheng1,‡, Joonwon Choi1,‡, Yongwoo Lee1, Seoyeong Lee1, Doyeon Lee1, and Min Jae Ko1,*

1 Department of Chemical Engineering, Hanyang University, Seoul, 04763, Republic of Korea

‡ These authors contributed equally: Wooyeon Kim, Jian Cheng, and Joonwon Choi

* Correspondence: mjko@hanyang.ac.kr (M. J. K.)

Fig. S1. Transmission electron microscopy (TEM) image of the TiO2 nanocrystals.

Fig. S2. Attenuated total reflectance–fourier transform infrared (ATR-FTIR) spectra of TiO2 films before and after ultraviolet (UV) sintering.

Fig. S3. X-ray diffraction (XRD) patterns of TiO2 film

Fig. S4. a–c Tauc plots and optical bandgap energies of SnO2, TiO2, and perovskite films. d–f Linear extrapolations of ultraviolet photoelectron spectroscopy (UPS) spectra for each sample.

| Sample | A1 (%) | τ1 (ns) | A2 (%) | τ2 (ns) | τave (ns) |
| --- | --- | --- | --- | --- | --- |
| Perovskite | 4.78 | 239.8 | 95.22 | 1569.63 | 1559.51 |
| SnO2 | 44.82 | 164.17 | 55.18 | 291.94 | 251.88 |
| SnO2 / TiO2 | 49.59 | 71.65 | 50.41 | 206.44 | 172.13 |

Table S1. Time constants calculated from time resolved photoluminescence (TRPL) spectra. Lifetime decay components were fitted using a bi-exponential decay model (Fit function = A1e-t/τ1+A2e-t/τ2).

τave=[(A1τ12+A2τ22)/(A1τ1+A2τ2)]

Fig. S5. Planar-view SEM images of the perovskite films on a SnO2 layer and b SnO2/TiO2 bilayer.

| ETL | VOC (V) | JSC (mA·cm−2) | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- |
| SnO2 | 1.19 | 22.87 | 83.04 | 22.66 |
| SnO2/TiO2 | 1.19 | 23.43 | 84.07 | 23.47 |

Table S2. Photovoltaic parameters of conventional glass/ITO substrate-based perovskite solar cells with various ETLs under 1 sun conditions.

Fig. S6. a J–V characteristics measured in both reverse (solid lines) and forward (dashed lines) directions of each ETL-based perovskite solar cell. b IPCE spectra of perovskite solar cells with difference ETLs and integrated JSC calculated from IPCE.

Fig. S7. Transmittance spectra of conventional glass/ITO (1100µm) and ultrathin glass (UTG)/ITO (50 µm).

| Substrate | VOC (V) | JSC (mA·cm−2) | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- |
| PEN | 1.18 | 22.01 | 69.42 | 18.00 |
| UTG | 1.17 | 22.13 | 58.44 | 15.18 |

Fig. S8. J−V curves and summarized photovoltaic parameters of polyethylene naphthalate (PEN)/ITO and UTG/ITO substrate-based PSCs.