Electronic Supporting Information (ESI)

Self-powered sensing platform for monitoring uric acid in sweat based on cobalt nanocrystal-graphene quantum dot-Ti3C2TX monolithic film electrode with excellent supercapacitor and sensing behavior

Li Ruiyi, Wei Mengyu, Zhou Xinyi, Li Zaijun* and Liu Xiaohao

Key Laboratory of Synthetic and Biological Colloids, Ministry of Education, School of Chemical and Material Engineering, School of Life Sciences and Health Engineering, Jiangnan University, Wuxi 214122, China

1. Experimental

1.1. Reagents and Materials

Cobalt Chloride (CoCl2) (99.99%), arginine, uric acid citric acid, and K4Fe(CN)6 (>99.95%) and were purchased from Sigma-Aldrich Company. Phosphate-buffered solution (PBS, Na2HPO4-NaH2PO4-KCl, 0.1 M, pH 7.4) was prepared in the laboratory. Polyvinyl alcohol (PVA) was purchased from Shanghai Macklin Biochemical Co., Ltd. Ti3AlC2 (400 mesh) was purchased from 11 Technology Co. Ltd. The PVA/H2SO4 gel electrolyte was prepared by adding 2 g of PVA in 20 mL of deionized water. Kept it at room temperature for 24 h and then heated at 95 C with stirring until a clear homogeneous solution was formed. Added 10 mL of 1 M H2SO4 solution under stirring and cool down to room temperature. The deionized (DI) water was produced by using Millipore Milli-Q grade with a resistivity of 18.2 MΩ cm-1.

1.2. GQD+ preparation

Arginine and citric acid was mixed with with a molar ratio of 1:1 and then heated at 160oC for 5 h. The formed GQD crude product was dissolved in water to produce a 100 mg·mL-1 of GQD solution. Followed by centrifugation at 10000 rpm for 2.5 min and dialysis. The collected solution was acidified to pH 1 by 1 M HCl solution and then freeze-dried to obtain solid GQD+ solid product.

1.3. Material characterization

Scanning electron microscope (SEM) analysis was carried out in HITACHI S-4800 field emission scanning electron microscope. Transmission electron microscope (TEM) images were conducted on a JEOL 2010plus transmission electron microscope at 200 keV. The sample was prepared by dispensing a small amount of dry powder in ethanol. Then, one drop of the suspension was dropped on 300 mesh copper. X-ray diffraction (XRD) pattern was measured on X-ray D8 Advance Instrument operated at 40 kV and 20 mA and using a Cu Kα radiation source with λ=0.15406 nm. X-ray photoelectron spectroscopy (XPS) was carried out in a PHI 5700 ESCA spectrometer with mono chromated Al KR radiation. Infrared spectrum (IR) was tested using Nicolet FT-IR 6700 spectrometer. Atomic force microscopic (AFM) images were taken by Multimode 8 Force Microscope (Bruker, Germany). UV-visible diffuse reflectance spectra (DRS) was measured on Shimadzu UV-3600 Plus. Zeta potential measurements were completed at ZetaPALS(Brookhaven Instruments, Inc).

1.4. Electrochemical measurements

Classical three-electrode system and symmetrical supercapacitor were prepared and used for examining the electrochemical properties of Co-GQD-Ti3C2TX film electrode. The three-electrode system includes one Co-GQD-Ti3C2TX film working electrode (1cm×1cm), one platinum foil (1cm×1cm) counter electrode, and one saturated calomel electrode reference electrode. The aqueous solution of 1 M H2SO4 was used as the electrolyte.

Cyclic voltammogram (CV), chronoamperometry, electrochemical impedance spectroscopy (EIS) and galvanostatic charge/discharge curves were carried on CHI 660D electrochemical workstation. The EIS measurements used the potential amplitude of ±5 mV and frequncy range of 0.01-105 Hz. The specific capacitances of three-electrode system and symmetrical supercapacitor were caluated using reported formula.

For the three-electrode testing system, the specific capacitance of single electrode (Cg) can be calculated by the equation (1) [1]. Here, Cg, I, m, V, and t present gravimetric capacitance (F g-1), current (A), active mass (g), potential range (V) and discharging time (s), respectively.

Cg=Itm∆V                                                                          (1)

For the symmetric supercapacitor, the specific capacitance (Cg2, F g-1), energy density (Eg, Wh kg-1), and power density (Pg, W kg-1) can be calculated by the equations (2), (3) and (4), respectively [1]. In the equation (2) and (3), the I, V and t are the current (A), mass (g) of active material (g), potential range (V) and discharging time (s), respectively.

Cg2=Itm∆V                                                                          (2)

Eg=Cg2ΔV22×3.6                                                                       (3)

Pg=Eg2×3600tdischarge                                                                (4)

2. Figures and Tables

Fig. s1 Scheme for construction of self-charging supercapacitor

Fig. s2 Optical photograph of electrochemical chip

Fig. s3 Scheme for synthesis of GQD+

Fig. s4 Optical photograph of the Ti3C2TX hydrogel containing 10%GQD+ (a) and 20%GQD+ (b) after centrifugation at 5000 rpm for 5 min

Fig. s5 AFM image of Ti3C2TX hydrogels

Fig. s6 Raman spectrum (A) and FTIR spectrum (B) of Co-GQD-Ti3C2TX film

Fig. s7 Nyquist plots of GQD, GQD-Ti3C2TX and Co-GQD-Ti3C2TX electrodes in 1.0 mM K4Fe(CN)6 in the PBS of pH 7.4. Inset: equivalent circuit from the EIS measurements

Fig. s8 CV curves at the scan rate of 10 mV s-1 (A) and chronoamperometry curves (B) of Co-GQD-Ti3C2TX film electrode in 1 M H2SO4 electrolyte within different potential ranges

Fig. s9 Charge-discharge curves (A) of three-electrode testing system at the current densities of 1, 2, 5, 7, 10, 15, 20, 25, 30, 35, 40, 45 and 50 A g-1 and the plot of specific capacitance vs. the current density

Fig. s10 DPV curves in 100 M uric acid at pH values of 5, 5.5, 6, 6.5, 7, 7.5, 8, 8.5 and 9 (A) and relationship curve between peak potential on the DPV curves and pH value (B)

Fig. s11 Absorption spectra of GQD+ at different pH values in the range from 5 to 9

Fig. s12 Peak currents for ten consecutive measurements

Fig. s13 Peak currents for different storage time

Fig. s14 Peak currents in different coexisting species

Table s1 comparison of supercapacitor behavior of MXene-based supercapacitors

| Electrode materials | Electrolyte | Test system | Specific capacitance at 1 A g-1 (F g-1) | Energy density (Wh kg-1) | Ref. |
| --- | --- | --- | --- | --- | --- |
| Blade coating MXene film | 3M H2SO4 | Three-electrode | 347 | / | [1] |
| Folded structured MXene film | 1M H2SO4 | Three-electrode | 345 | / | [2] |
|  | PVA/H2SO4 | Symmetrical supercapacitor | / | 14.1 |  |
| MXene/polyaniline film | 1M H2SO4 | Three-electrode | 661 | / | [3] |
|  | PVA/H2SO4 | Symmetrical supercapacitor | 146.4 | 17.5 |  |
| MXene/graphene film | 1M H2SO4 | Three-electrode | 337.4 | / | [4] |
|  | PVA/H2SO4 | Symmetrical supercapacitor | 63.6 | 19.7 |  |
| Ti3C2TX/carbon nanotube/CuS Film | PVA/H2SO4 | Symmetrical supercapacitor | 336.7 | 12.7 | [5] |
| Porous polypyrrole/Ti3C2TX/alginate aerogel | 2M H2SO4 | Three-electrode | 457 |  | [6] |
|  | 2M H2SO4 | Symmetrical supercapacitor | 200 mF cm-2 |  |  |
| Modified Ti3C2TX with hyperbranched polyethylene ionomers | EMIMBF4 | Symmetrical supercapacitor | 220 |  | [7] |
| Co-GQD-Ti3C2TX | 1M H2SO4 | Three-electrode | 715 F g-1 at 1 A g-1 and 528 F g-1 at 10 A g-1 |  | This Work |
|  | PVA/H2SO4 | Symmetrical supercapacitor (without current collector, conductive agent and binder) | 296 F g-1 at 1A g-1 and 180 F g-1 at 10 A g-1 | 29.6 W h kg-1 at 299.9 W kg-1 |  |

References

[1]	H.X. Ma, J.Q. Wang, J.F. Wang, S.K. Shang, Y. Yang, Z.W. Fan, Blade-coated Ti3C2TX MXene films for pseudocapacitive energy storage and infrared stealth, Diamond and Related Materials 131 (2023) 109587.

[12]	Z.M. Fan, J.F. Wang, H. Kang H, Y.S. Wang, Z.M. Xie, Z.J. Cheng, Y.Y. Liu, A compact MXene film with folded structure for advanced supercapacitor electrode material, ACS Applied Energy Materials 3 (2020) 1811-1820.

[3]	C.L. Li, S. Wang, Y.H. Cui, X.D. Wang, Z.P. Wang, D. Liang, Y. Chi, Z. Wang, Sandwich-like high-load MXene/polyaniline film electrodes with ultrahigh volumetric capacitance for flexible supercapacitors, Journal of Colloid and Interface Science 2022, 620: 35-46.

[4]	Y.B. Wang, N.J. Chen, Y. Liu, X.F. Zhou, B. Pu, Y. Qing, M.Z. Zhang, X.L. Jiang, J.F. Huang, Q. Tang, B. Zhou, W.Q. Yang, MXene/graphdiyne nanotube composite films for free-Standing and flexible Solid-State supercapacitor, Chemical Engineering Journal 450 (2022) 138398.

[5]	A.L. Dang, Y.T. Sun, Y.H. Liu, Y. Xia, X. Liu, Y.L. Gao, S.H. Wu,T,H. Li, A. Zada, F. Ye, Flexible Ti3C2TX/Carbon nanotubes/CuS film electrodes based on a dual-Structural design for high-performance all-solid-state supercapacitors, ACS Applied Energy Materials 5 (2022) 9158-9172.

[6]   X. Wu, J. Li, Y. Zhu, W. Cai, J. Xu, Y. Qin, Y. Kong, Porous polypyrrole/Ti3C2TX/alginate aerogels prepared by sacrificial template strategy as electrode materials in symmetric supercapacitors, Journal of Energy Storage 66 (2023) 107483.

[7]   B. Raisi, L. Huang, Z. Ye, Modification of Ti3C2Tx MXene with hyperbranched polyethylene ionomers: stable dispersions in nonpolar/low-polarity organic solvents, oxidation protection, and potential application in supercapacitors, J. Mater. Chem. A 11 (2023) 17167-17187.

References

[1] C. Li, J. Wang, Y. Yan, P. Huo, X. Wang, MOF-derived NiZnCo-P nano-array for asymmetric supercapacitor, Chem. Eng. J. 446 (2022) 137108, https://doi.org/10.1016/j.cej.2022.137108.