Supplementary materials

Table 1 shows the basic mechanical parameters of the studied experimental subject, which were obtained from the roof sandstone of a mine in Shandong, China.

Table 1 Basic parameters of rock samples

| Rock samples number | Diameter | Height | Mass | Density | Wave velocity |
| --- | --- | --- | --- | --- | --- |
|  | (mm) | (mm) | (g) | (g/cm3) | (m/s) |
| R1 | 49.80 | 99.50 | 455.0 | 2.348 | 2538 |
|  | 49.82 | 99.50 |  | 2.346 | 2513 |
|  | 49.80 | 99.52 |  | 2.347 | 2488 |
| R2 | 49.78 | 99.52 | 457.5 | 2.362 | 2415 |
|  | 49.82 | 99.54 |  | 2.358 | 2488 |
|  | 49.80 | 99.52 |  | 2.360 | 2415 |
| R3 | 49.82 | 99.52 | 457.1 | 2.356 | 2463 |
|  | 49.82 | 99.54 |  | 2.356 | 2463 |
|  | 49.80 | 99.56 |  | 2.357 | 2513 |
| R4 | 49.80 | 99.40 | 454.8 | 2.349 | 2538 |
|  | 49.80 | 99.42 |  | 2.349 | 2488 |
|  | 49.82 | 99.44 |  | 2.346 | 2513 |
| R5 | 49.82 | 99.42 | 453.9 | 2.342 | 2463 |
|  | 49.78 | 99.40 |  | 2.346 | 2489 |
|  | 49.80 | 99.44 |  | 2.343 | 2439 |

The correlation coefficients, permutation entropy, and variance contribution rates for the IMF components of SIG2-2, SIG2-3 and SIG2-4 are illustrated in Tables 2-4.

Table 2 Correlation coefficients, permutation entropy, and variance contribution rates for the IMF components of SIG2-2

| Components | IMF1 | IMF2 | IMF3 | IMF4 | IMF5 | IMF6 | IMF7 | IMF8 | IMF9 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Correlation coefficients | 0.127 | 0.354 | 0.201 | 0.138 | 0.124 | 0.682 | 0.672 | 0.471 | 0.183 |
| Permutation entropy | 0.905 | 0.555 | 0.381 | 0.312 | 0.208 | 0.135 | 0.126 | 0.117 | 0.081 |
| Variance contri- bution rates | 0.000 | 0.095 | 0.011 | 0.005 | 0.017 | 0.111 | 0.307 | 0.180 | 0.043 |

Table 3 Correlation coefficients, permutation entropy, and variance contribution rates for the IMF components of SIG2-3

| Components | IMF1 | IMF2 | IMF3 | IMF4 | IMF5 | IMF6 | IMF7 | IMF8 | IMF9 | IMF10 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Correlation coefficients | 0.332 | 0.602 | 0.436 | 0.364 | 0.330 | 0.545 | 0.340 | 0.048 | 0.055 | 0.034 |
| Permutation entropy | 0.878 | 0.512 | 0.380 | 0.302 | 0.205 | 0.153 | 0.120 | 0.118 | 0.114 | 0.070 |
| Variance contri- bution rates | 0.006 | 0.232 | 0.079 | 0.095 | 0.052 | 0.253 | 0.071 | 0.025 | 0.001 | 0.000 |

Table 4 Correlation coefficients, permutation entropy, and variance contribution rates for the IMF components of SIG2-4

| Components | IMF1 | IMF2 | IMF3 | IMF4 | IMF5 | IMF6 | IMF7 | IMF8 | IMF9 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Correlation coefficients | 0.057 | 0.479 | 0.520 | 0.481 | 0.525 | 0.303 | 0.344 | 0.138 | 0.030 |
| Permutation entropy | 0.905 | 0.553 | 0.375 | 0.273 | 0.193 | 0.150 | 0.132 | 0.118 | 0.110 |
| Variance contri- bution rates | 0.004 | 0.088 | 0.107 | 0.152 | 0.192 | 0.132 | 0.142 | 0.026 | 0.013 |

The specific decomposition principle of the ICEEMDAN algorithm is as follows:

(1) Let the original signal be x[n]. Define the operator Ek(*) to represent the k-th intrinsic mode function (IMF) obtained from Empirical Mode Decomposition (EMD), define the operator M(*) to represent the local mean of the signal, and define the operator <*> to represent taking the mean. According to EMD, E1(x) = x[n] − M(x).

(2) Construct x(i) = x[n] + ε0E1(wi[n]),

where wi[n] represents the i-th added white noise, and ε0 is the noise standard deviation.

(3) Calculate the local mean M(x(i)) of x(i) and take the mean to obtain the first residual component r1[n] = < M(x(i))>.

(4) Calculate the first intrinsic mode function IMF1: IMF1 = x[n] - r1[n].

(5) Calculate the second intrinsic mode function IMF2: IMF2 = r1[n] - r2[n],

where r2[n] = < M(r1[n] + ε1E2(wi[n])>.

(6) Using the formula IMF2 = rk−1[n] - rk[n], calculate the value of the kth intrinsic mode function IMFk.

where rk[n] = < M(rk−1[n] + εk-1Ek(wi[n])>, for k = 2, 3, …, N.

Figure 1 Principle of the ICEEMDAN Algorithm

The relationship between correlation coefficient, permutation entropy, and their respective thresholds for the components of SIG2-2, SIG2-3, and SIG2-4 are illustrated in Figures 2-4.

| Figure 2 The relationship between (a) correlation coefficient, (b) permutation entropy, and their respective thresholds for the components of SIG2-2 |  |
| --- | --- |
| Figure 3 The relationship between (a) correlation coefficient, (b) permutation entropy, and their respective thresholds for the components of SIG2-3 |  |
| Figure 4 The relationship between (a) correlation coefficient, (b) permutation entropy, and their respective thresholds for the components of SIG2-4 |  |