Supporting Information

Excellent Electromagnetic Interference Shielding of Multi-layered Thermoplastic Polyurethane Nanocomposites with CoFe2O4 Nanoparticles and Graphite

Nithiya Hanna Wilson, Anju, Milan Masař, Michal Machovský, David Škoda, Pavel Urbánek, Michal Urbánek, Marek Pöschl, Jarmila Vilčáková, Ivo Kuřitka, Raghvendra Singh Yadav*

Centre of Polymer Systems, University Institute, Tomas Bata University in Zlin, Trida Tomase Bati 5678, 760 01 Zlin, Czech Republic

*Corresponding author: yadav@utb.cz , Tel.: +420576031725

Fig. S1 Schematic representation of the synthesis of CoFe2O4 NPs by sonochemical approach.

| (a) | (b) | (c) |
| --- | --- | --- |

Fig. S2 FE-SEM surface images of (a) TPU, (b) F/F/F, and (c) G/G/G.

Fig. S3 EDX spectra of (a) TPU, (b) F/F/F, (c) G/G/G, (d) F/G/F, and (e) G/F/G.

Table S1 The percentage compositions of carbon, oxygen, iron, and cobalt in TPU and TPU-based multi-layered nanocomposites.

| Sample/Material | C % | O % | Fe % | Co % |
| --- | --- | --- | --- | --- |
| TPU | 86.2 | 10.7 | - | - |
| FFF-TPU | 37.0 | 19.0 | 27.0 | 13.0 |
| GGG-TPU | 90.3 | 9.3 | - | - |
| FGF-TPU | 50.0 | 20.0 | 18.0 | 9.0 |
| GFG-TPU | 66.0 | 12.0 | 12.0 | 6.0 |

Fig. S4 FT-IR spectra of (a) CoFe2O4 NPs and graphite, (b) TPU and its multi-layered nanocomposites F/F/F, G/G/G, F/G/F, and G/F/G.

Fig. S5 Raman spectra of (a) CoFe2O4 NPs, (b) graphite, (c) TPU and its multi-layered nanocomposites F/F/F, G/G/G, F/G/F, and G/F/G.

Fig. S6 Contact angle images of (a) TPU and (b) G/F/G.