Effect of process variable on production of thermoplastic vulcanizates based on SEBS/PP/LLDPE via reactive extrusion

Mehri Dana1,2, Mohammad Reza Nabid1,*, Gholam Hossein Zohuri3,4,*, Saeid Asadi Shahidi2, Sohail Yazdanbakhsh2

1Department of Polymer & Materials Chemistry, Faculty of Chemistry and Petroleum Science, Shahid Beheshti University, GC, 1983969411Tehran, Iran.

2Department of Materials Engineering, Pouya Gostar Khorasan Co. of Part Lastic Group, Mashhad, Iran.

3Department of Chemistry, Faculty of Science, Ferdowsi University of Mashhad, Mashhad, Iran.

4Environmental Chemistry Research Centre, Department of Chemistry, Faculty of Science, Ferdowsi University of Mashhad, Mashhad, Iran.

Correspondence to: Mohammad Reza Nabid (m-nabid@sbu.ac.ir ), Gholam Hossein Zohuri (zohuri@um.ac.ir )

- A comprehensive experimental study was performed to identify the optimal process conditions for the production of the TPVs based on SEBS/PP/LLDPE.

- the properties of the prepared TPV via the two-step method are superior to the one-step method.

- the properties of the prepared TPV by the method B are superior to the method A.

- In investigating the effect of process temperature (210-230 °C, 170-190 °C, 150-170 °C and 140-160 °C), According to the observed result of properties of the TPV and of its surface quality improvement in the temperature profile of 140-160 °C, this temperature was chosen as the optimal temperature profile.

- Due to the increase in speeds of the twin screw extruder (from 180 to 250 rpm) in 140-160 °C, surface quality was suitable and smooth.