TABLE S1. Orthogonal range analysis results

| Statistical parameters | Pressing time | Pressing temperature | Concentration | Retardant |
| --- | --- | --- | --- | --- |
|  | a | b | c | d |
| Modulus of elasticity |  |  |  |  |
| K1 | 49069.74 | 47797.69 | 48076.33 | 49097.72 |
| K2 | 48436.21 | 49708.25 | 49429.62 | 48408.22 |
| k1 | 12267.43 | 11949.42 | 12019.08 | 12274.43 |
| k2 | 12109.05 | 12427.06 | 12357.40 | 12102.06 |
| R | 158.38 | 477.64 | 338.32 | 172.38 |
| Optimal level | a2 | b2 | c2 | d1 |
| Modulus of rapture |  |  |  |  |
| K1 | 372.99 | 362.96 | 387.14 | 378.61 |
| K2 | 379.84 | 389.87 | 365.69 | 374.22 |
| k1 | 93.25 | 90.74 | 96.79 | 94.65 |
| k2 | 94.96 | 97.47 | 91.42 | 93.56 |
| R | 1.71 | 6.73 | 5.36 | 1.10 |
| Optimal level | a2 | b2 | c1 | d1 |
| Horizontal shear strength |  |  |  |  |
| K1 | 28.68 | 29.80 | 30.23 | 28.72 |
| K2 | 29.73 | 28.62 | 28.18 | 29.73 |
| k1 | 7.17 | 7.45 | 7.56 | 7.18 |
| k2 | 7.43 | 7.15 | 7.05 | 7.43 |
| R | 0.26 | 0.30 | 0.51 | 0.25 |
| Optimal level | a2 | b1 | c1 | d2 |
| Compressive strength |  |  |  |  |
| K1 | 207.99 | 211.16 | 214.10 | 214.74 |
| K2 | 212.81 | 209.65 | 206.70 | 206.07 |
| k1 | 52.00 | 52.79 | 53.53 | 53.68 |
| k2 | 53.20 | 52.41 | 51.68 | 51.52 |
| R | 1.20 | 0.38 | 1.85 | 2.17 |
| Optimal level | a2 | b1 | c1 | d1 |
| Limiting Oxygen Index |  |  |  |  |
| K1 | 128.33 | 129.23 | 125.17 | 131.67 |
| K2 | 128.73 | 127.83 | 131.90 | 125.40 |
| k1 | 32.08 | 32.31 | 31.29 | 32.92 |
| k2 | 32.18 | 31.96 | 32.98 | 31.35 |
| R | 0.10 | 0.35 | 1.68 | 1.57 |
| Optimal level | a2 | b1 | c2 | d1 |
| Fireproof time |  |  |  |  |
| K1 | 3876.00 | 4144.33 | 3722.67 | 4297.33 |
| K2 | 4036.33 | 3768.00 | 4189.67 | 3615.00 |
| k1 | 969.00 | 1036.08 | 930.67 | 1074.33 |
| k2 | 1009.08 | 942.00 | 1047.42 | 903.75 |
| R | 40.08 | 94.08 | 116.75 | 170.58 |
| Optimal level | a2 | b1 | c2 | d1 |

TABLE S2. Results of variance analysis

| Property | Source |  | Mean Sq. | F | p-value |
| --- | --- | --- | --- | --- | --- |
| Modulus of elasticity (MOE) | Pressing time |  | 150508.5 | 0.815 | 0.378 |
|  | Pressing temperature |  | 1368839.8 | 7.409 | 0.014* |
|  | Concentration |  | 686769.3 | 3.717 | 0.069 |
|  | Type of retardant |  | 178278.8 | 0.965 | 0.338 |
|  | Error |  | 184754.0 | — | — |
| Modulus of raptures (MOR) | Pressing time |  | 17.6 | 0.234 | 0.634 |
|  | Pressing temperature |  | 271.4 | 3.603 | 0.073 |
|  | Concentration |  | 172.6 | 2.292 | 0.147 |
|  | Type of retardant |  | 7.2 | 0.096 | 0.760 |
|  | Error |  | 75.3 | — | — |
| Horizontal shear strength (HSS) | Pressing time |  | 0.4 | 1.427 | 0.247 |
|  | Pressing temperature |  | 0.5 | 1.813 | 0.194 |
|  | Concentration |  | 1.6 | 5.440 | 0.031* |
|  | Type of retardant |  | 0.4 | 1.427 | 0.247 |
|  | Error |  | 0.3 | — | — |
| Compressive strength (CS) | Pressing time |  | 8.7 | 2.750 | 0.114 |
|  | Pressing temperature |  | 0.9 | 0.269 | 0.610 |
|  | Concentration |  | 20.5 | 6.489 | 0.020* |
|  | Type of retardant |  | 28.2 | 8.930 | 0.008** |
|  | Error |  | 3.2 | — | — |
| Limiting Oxygen Index (LOI) | Pressing time |  | 0.1 | 0.194 | 0.665 |
|  | Pressing temperature |  | 0.7 | 2.371 | 0.140 |
|  | Concentration |  | 17.0 | 54.844 | 0.000** |
|  | Type of retardant |  | 14.7 | 47.505 | 0.000** |
|  | Error |  | 0.3 | — | — |
| Fireproof time (FT) | Pressing time |  | 9640.0 | 5.709 | 0.027* |
|  | Pressing temperature |  | 53110.0 | 31.452 | 0.000** |
|  | Concentration |  | 81783.4 | 48.433 | 0.000** |
|  | Type of retardant |  | 174592.0 | 103.394 | 0.000** |
|  | Error |  | 1688.6 | — | — |