Supplemental material

Polypyrrole deposited on the core-shell structured nitrogen doped porous carbon@Ag-MOF for signal amplification detection of chloride ions

Xiurong Zhai a, *, Qian Li b, Yang Cao c, Mengjie Han a, Hailian Sun a , Lelin Du, Xiyun Yang a, Yuxin Wei a, Congcong Yu a

a College of Chemistry, Chemical Engineer and Materials, Jining University, Qufu City, Shandong Province, 273155, PR China

b School of Chemistry and Chemical Engineering, Yangzhou University, Yangzhou, Jiangsu, 225009, P. R. China

c Ecological and Environmental Affairs Center of Jining City, Jining City, Shandong Province, 272000 PR China

* Corresponding Authors, E-mail addresses: zhaixiurong@163.com

Fig. S1. The stability of NC@Ag-MOF-PPy-modified electrodes upon continuous LSV scanning for four times in buffer solution (0.1 M, pH 7.0) at the scan rate of 100 mV/ s.

Fig. S2 The electrochemical LSV responses of NC@Ag-MOF-PPy-modified electrodes to Cl- ions (10 mM) depending on (a) the volumes of pyrrole, (b) pH values, and (c) reaction time for the signal outputs of solid-state AgCl.

Fig. S3 (a) The electroanalytical reproducibility of six different NC@Ag-MOF-PPy-modified electrodes for detecting 10 mM Cl- ions. (b) Stability tests of NC@Ag-MOF-PPy-modified electrodes stored over 30 days

Fe

N

Ag

.

Table S1 Recovery test results of the developed electroanalysis method in sensing Cl- ions in the samples of human serum and urine (n=3).

| Sample | Spiked Cl- ions (mM) | Founded Cl- ions (mM) | Recovery (%) |
| --- | --- | --- | --- |
| Human serum | 0 | 102 | ---- |
|  | 30 | 130 | 93.3 |
|  | 60 | 159 | 95.0 |
| Human urine | 0 | 175 | --- |
|  | 30 | 208 | 110.0 |
|  | 60 | 232 | 95.0 |