Supplementary information

for

The Effectiveness of TRIS and Ammonium buffers in Glass Dissolution Studies: A Comparative Analysis

Ramya Ravikumar,1  Clare L. Thorpe,1 Claire L. Corkhill,2  Samual A. Walling,1 James J. Neeway,3 Carolyn I. Pearce,3 Albert A. Kruger,4 David S. Kosson, 5 Jose Marcial,3 and Russell J. Hand 1

1 Department of Materials Science and Engineering, University of Sheffield, Sheffield, United Kingdom

2 School of Earth Sciences, University of Bristol, Bristol, United Kingdom.

3 Pacific Northwest National Laboratory, Richland, Washington

4 Office of River Protection, U.S. Department of Energy, Richland, Washington

5 Department of Civil and Environmental Engineering, Vanderbilt University and CRESP Nashville, Tennessee

| Table of contents |  | Page No |
| --- | --- | --- |
| Figure 1 | Organic buffers of varying pH scale in neutral to alkaline regime | S1 |
| Figure 2 | NLi vs. time for LAWA44 in pH ≈ 8.5 of varying concentration of TRIS–HNO3 solution | S2 |
| Figure 3 | pH as a function of time for LAWA44 in pH ≈ 8.5, 9.5 and 10.5 of 0.1M Tris–HNO3 solution at RT, 40 °C and 60 °C ( set pH value, ★ pH measured for blank solution [0.1 MTris–HNO3]) | S3 |
| Figure 4 | Powder XRD patterns of LAW A44 (before and after dissolution) in pH ≈ 10.5 of 0.1M TRIS–HNO3 solution at 60 °C | S4 |
| Figure 5 | 11B NMR spectra of the as-prepared H3BO3 solutions at RT with pH of 7.5, 8.5, 9.5 and 10.5 | S5 |
| Figure 6 | 11B NMR spectra of the as-prepared 1:1 Tris/boron solutions at RT with pH of 8.5, 9.5 and 10.5 | S6 |
| Figure 7 | 11B NMR spectra of the as-prepared 1:1 Tris/boron solutions at 40 °C with pH of 8.5, 9.5 and 10.5 | S7 |
| Figure 8 | 11B NMR spectra of the as-prepared 1:1 Tris/boron solutions at 60 °C with pH of 8.5, 9.5 and 10.5 | S8 |
| Figure 9 | NLi as a function of time for LAWA44 in pH ≈ 8.5 of varying concentration of NH3/NH4Cl solution | S9 |
| Figure 10 | pH as a function of time for LAWA44 in pH ≈ 8.5, 9.5 and 10.5 of 0.1M NH3/NH4Cl buffered solution at RT, 40 °C and 60 °C ( set pH value, ★ pH measured for blank solution [0.1M NH3/NH4Cl]) | S10 |
| Figure 11 | NLi ( Na, B, Si, Al ) as a function of time for LAW A44 glass in Type I water at 18 ± 1 °C, 40 °C, and 60 °C | S11 |
| Figure 12 | 11B NMR spectra of the of the aliquot leachate collected on day 8 of dissolution experiments at RT with set pH of 8.5, 9.5 and 10.5 using ammonia buffer. | S12 |
| Figure 13 | Normalised boron dissolution rates as a function of temperature for LAW A44 at pH 8.5,9.5 and 10.5 in (left) Tris buffer and (right) NH3/NH4Cl buffer and at (top) time duration of 15min to 8 days, (middle) 15 mins to 8 hours and (bottom) 1 day to 4 days. Solid lines represent the fitting for the linear regression. | S13 |
| Table 1 | ICP-OES elemental concentration data for LAWA44 powder altered in varying concentrations of TRIS/HNO3 solution. | S14 |
| Table 2 | Normalised mass loss (g m-2) for Al, B, Na and Si from LAWA44 powder altered in varying concentrations of TRIS/HNO3 solution | S15 |
| Table 3 | Average pH during the 8-day for LAWA44 powder altered in varying concentrations of TRIS/HNO3 solution. | S16 |
| Table 4 | ICP-OES elemental concentration data for LAW A44 glass powders altered in 0.1 M TRIS-HNO3 /LAW A44. | S17-21 |
| Table 5 | Normalised mass loss (g m-2) for Al, B, Na and Si from LAWA44 powder altered in 0.1 M TRIS/HNO3 solution at a target pH of 8.5 and temperatures of RT, 40 oC and 60 oC. | S22 |
| Table 6 | Normalised mass loss (g m-2) for Al, B, Na and Si from LAWA44 powder altered in 0.1 M TRIS/HNO3 solution at a target pH of 9.5 and temperatures of RT, 40 oC and 60 oC. | S23 |
| Table 7 | Normalised mass loss (g m-2) for Al, B, Na and Si from LAWA44 powder altered in 0.1 M TRIS/HNO3 solution at a target pH of 10.5 and temperatures of RT, 40 oC and 60 oC. | S24 |
| Table 8 | ICP-OES elemental concentration data for LAWA44 powder altered in varying concentrations of NH4Cl/NH3 solution. | S25 |
| Table 9 | Normalised mass loss (g m-2) for Al, B, Na and Si from LAWA44 powder altered in varying concentrations of NH4Cl/NH3 solution. | S26 |
| Table 10 | Average pH during the 8-day for LAWA44 powder altered in varying concentrations of NH3/NH4Cl solution | S27 |
| Table 11 | ICP-OES elemental concentration data for LAWA44 glass powders altered in 0.1 M NH4Cl-NH3/LAW A44. | S28-31 |
| Table 12 | Normalised mass loss (g m-2) for Al, B, Na and Si from LAWA44 powder altered in 0.1 M NH4Cl/NH3 solution at target pH 8.5 and temperatures of RT, 40 oC and 60 oC. | S32 |
| Table 13 | Normalised mass loss (g m-2) for Al, B, Na and Si from LAWA44 powder altered in 0.1 M NH4Cl/NH3 solution at target pH 9.5 and temperatures of RT, 40 oC and 60 oC. | S33 |
| Table 14 | Normalised mass loss (g m-2) for Al, B, Na and Si from LAWA44 powder altered in 0.1 M NH4Cl/NH3 solution at target pH 10.5 and temperatures of RT, 40 oC and 60 oC. | S34 |
| Table 15 | Activation energy calculated using linear regression of normalised boron dissolution rates as a function of temperature for LAWA44 at varying pH. | S35 |
| Table 16 | Composition of LAWA44 glass in oxide wt %. | S36 |

Figure 1. Organic buffers of varying pH scale in neutral to alkaline regime (Ferriera et al., 2015) 18

Figure 2. NLi as a function of time for LAWA44 in pH 8.5 of varying concentration of TRIS–HNO3 solution. Error bars represent the standard deviation of duplicate measurements.

Figure 3. pH as a function of time for LAWA44 in pH ≈ 8.5, 9.5 and 10.5 of 0.1M Tris–HNO3 solution at RT, 40 °C and 60 °C (   set pH value,   ★  pH measured for blank solution [0.1 MTris–HNO3]).

Figure 4. Powder XRD patterns of LAWA44 (before and after dissolution) in pH ≈ 10.5 of 0.1 M Tris–HNO3 solution at 60 °C.

Fig S6. FT-IR spectra of LAWA44 Day 8 sample (before and post dissolution) in pH ≈ 10.5 of 0.1M Tris–HNO3 solution at 60 °C

Figure 5. 11B NMR spectra of the as-prepared H3BO3 solutions at room temperature (RT) with pH of 7.5, 8.5, 9.5 and 10.5.

Figure 6. 11B NMR spectra of the as-prepared 1:1 Tris/boron solutions at room temperature (RT) with pH of 8.5, 9.5 and 10.5.

Figure 7. 11B NMR spectra of the as-prepared 1:1 Tris/boron solutions at 40 °C with pH of 8.5, 9.5 and 10.5.

Figure 8. 11B NMR spectra of the as prepared 1:1 Tris/boron solutions at 60 °C with pH of 8.5, 9.5 and 10.5.

Figure 9. NLi as a function of time for LAWA44 in pH ≈ 8.5 of varying concentration of NH3/NH4Cl solution.

Figure 10. pH as a function of time for LAWA44 in pH ≈ 8.5, 9.5 and 10.5 of 0.1M NH3/NH4Cl buffered solution at RT, 40 °C and 60 °C (   set pH value, ★ pH measured for blank solution [0.1M NH3/NH4Cl]).

Figure 11. NLi ( Na,   B,    Si,   Al )  as a function of time for the LAWA44 glass in Type I water at RT, 40 °C, and 60 °C.

Figure 12. 11B NMR spectra of the of the aliquot leachate collected on day 8 of dissolution experiments at RT with set pH of 8.5, 9.5 and 10.5 using ammonia buffer.

Figure 13. Normalised boron dissolution rates as a function of temperature for LAW A44 at pH 8.5,9.5 and 10.5 in (left) Tris buffer and (right) NH3/NH4Cl buffer and at (top) time duration of 15min to 8 days, (middle) 15 mins to 8 hours and (bottom) 1 day to 4 days. Solid lines represent the fitting for the linear regression.

Table 1. ICP-OES elemental concentration data for LAWA44 powder altered in varying concentrations of TRIS/HNO3  solution

|  |  |  | Average elemental concentration across duplicates |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Sample | Temperature (°C) | Set pH | Time (Days) | Al (ppm) | B(ppm) | Na (ppm) | Si (ppm) |
| 0.02 M TRIS/ LAW A44 | RT | 8.58 | 1 | 0.11 ± 0.01 | 0.88 ± 0.01 | 10.63 ± 0.04 | 1.46 ± 0.01 |
|  |  |  | 2 | 0.19 ± 0.02 | 1.07 ± 0.11 | 12.94 ± 1.10 | 2.32 ± 0.26 |
|  |  |  | 3 | 0.23 ± 0.01 | 1.08 ± 0.02 | 13.59 ± 0.28 | 2.66 ± 0.01 |
|  |  |  | 4 | 0.27 ± 0.01 | 1.15 ± 0.05 | 14.65 ± 0.18 | 3.12 ± 0.02 |
|  |  |  | 8 | 0.49 ± 0.00 | 1.46 ± 0.04 | 19.99 ±0.47 | 5.09 ± 0.07 |
| 0.05 M TRIS / LAW A44 | RT | 8.58 | 1 | 0.11 ± 0.00 | 0.94 ± 0.02 | 10.27 ± 0.04 | 1.44 ± 0.01 |
|  |  |  | 2 | 0.19 ± 0.00 | 0.95 ± 0.07 | 11.97 ± 0.13 | 2.01 ± 0.01 |
|  |  |  | 3 | 0.23 ± 0.01 | 0.99 ± 0.06 | 12.74 ± 0.22 | 2.45 ± 0.01 |
|  |  |  | 4 | 0.27 ± 0.02 | 1.12 ± 0.05 | 14.40 ± 0.21 | 2.95 ± 0.00 |
|  |  |  | 8 | 0.48 ± 0.01 | 1.27 ± 0.01 | 18.36 ± 0.35 | 4.86 ± 0.03 |
| 0.1 M TRIS / LAW A44 | RT | 8.56 | 1 | 0.15 ± 0.01 | 0.81 ± 0.00 | 10.04 ±0.01 | 1.37 ± 0.01 |
|  |  |  | 2 | 0.20 ± 0.00 | 0.94 ± 0.01 | 11.70 ± 0.20 | 1.92 ± 0.01 |
|  |  |  | 3 | 0.26 ± 0.00 | 1.01 ± 0.01 | 13.28 ± 0.13 | 2.50 ± 0.03 |
|  |  |  | 4 | 0.30 ± 0.02 | 1.09 ± 0.01 | 14.21 ± 0.17 | 2.85 ± 0.09 |
|  |  |  | 8 | 0.68 ± 0.06 | 1.27 ± 0.01 | 18.62 ± 0.14 | 4.97 ±0.07 |
| 0.3 M TRIS / LAW A44 | RT | 8.58 | 1 | 0.19 ± 0.00 | 0.75 ± 0.02 | 9.17 ± 0.12 | 1.40 ± 0.01 |
|  |  |  | 2 | 0.24 ± 0.00 | 0.83 ± 0.01 | 10.53 ± 0.16 | 1.97 ± 0.05 |
|  |  |  | 3 | 0.31 ± 0.01 | 0.94 ± 0.01 | 11.95 ± 0.18 | 2.54 ± 0.05 |
|  |  |  | 4 | 0.32 ± 0.01 | 1.00 ± 0.01 | 12.71 ± 0.06 | 2.80 ± 0.06 |
|  |  |  | 8 | 0.57 - | 1.16 - | 16.45 - | 4.73 - |

Table 2. Normalised mass loss (g m-2) for Al, B, Na and Si from LAWA44 powder altered in varying concentrations of TRIS/HNO3  solution

|  | Average normalised mass loss (g m-2) of elements from LAW A44 in 0.02 M TRIS buffer |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Time (days) | Al | Standard deviation | B | Standard deviation | Na | Standard deviation | Si | Standard deviation |
| 1 | 1.60E-03 | 1.32E-04 | 1.48E-02 | 6.27E-05 | 3.33E-02 | 7.84E-05 | 3.77E-03 | 1.03E-05 |
| 2 | 2.86E-03 | 2.07E-04 | 1.78E-02 | 1.26E-03 | 4.06E-02 | 2.43E-03 | 5.98E-03 | 4.82E-04 |
| 3 | 3.42E-03 | 5.13E-05 | 1.81E-02 | 3.26E-04 | 4.26E-02 | 6.12E-04 | 6.84E-03 | 1.42E-05 |
| 4 | 3.99E-03 | 9.46E-05 | 1.92E-02 | 5.93E-04 | 4.60E-02 | 4.08E-04 | 8.03E-03 | 4.38E-05 |
| 8 | 7.17E-03 | 3.08E-05 | 2.44E-02 | 4.60E-04 | 6.27E-02 | 1.05E-03 | 1.31E-02 | 1.21E-04 |
|  | Average normalised mass loss (g m-2) of elements from LAW A44 in 0.05 M TRIS buffer |  |  |  |  |  |  |  |
| 1 | 1.65E-03 | 2.93E-06 | 1.57E-02 | 2.48E-04 | 3.22E-02 | 7.84E-05 | 3.70E-03 | 1.80E-05 |
| 2 | 2.73E-03 | 1.61E-05 | 1.58E-02 | 8.15E-04 | 3.75E-02 | 2.98E-04 | 5.19E-03 | 1.80E-05 |
| 3 | 3.42E-03 | 1.11E-04 | 1.65E-02 | 7.02E-04 | 3.99E-02 | 4.86E-04 | 6.32E-03 | 1.55E-05 |
| 4 | 3.98E-03 | 1.88E-04 | 1.87E-02 | 6.43E-04 | 4.52E-02 | 4.70E-04 | 7.60E-03 | 6.44E-06 |
| 8 | 7.05E-03 | 6.75E-05 | 2.13E-02 | 1.17E-04 | 5.76E-02 | 7.68E-04 | 1.25E-02 | 5.80E-05 |
|  | Average normalised mass loss (g m-2) of elements from LAW A44 in 0.1 M TRIS buffer |  |  |  |  |  |  |  |
| 1 | 2.18E-03 | 1.31E-04 | 1.35E-02 | 9.19E-06 | 3.15E-02 | 1.57E-05 | 3.54E-03 | 3.54E-03 |
| 2 | 2.91E-03 | 3.74E-05 | 1.57E-02 | 1.63E-04 | 3.67E-02 | 4.39E-04 | 4.94E-03 | 4.94E-03 |
| 3 | 3.83E-03 | 4.18E-05 | 1.68E-02 | 1.75E-04 | 4.16E-02 | 2.98E-04 | 6.45E-03 | 6.45E-03 |
| 4 | 4.41E-03 | 1.67E-04 | 1.81E-02 | 1.34E-04 | 4.46E-02 | 3.76E-04 | 7.33E-03 | 7.33E-03 |
| 8 | 1.00E-02 | 5.81E-04 | 2.13E-02 | 1.00E-04 | 5.84E-02 | 3.14E-04 | 1.28E-02 | 1.28E-02 |
| Time (days) | Average normalised mass loss (g m-2) of elements from LAW A44 in 0.3 M TRIS buffer |  |  |  |  |  |  |  |
| 1 | 2.78E-03 | 2.64E-05 | 1.25E-02 | 2.06E-04 | 2.88E-02 | 2.62E-04 | 3.60E-03 | 9.02E-06 |
| 2 | 3.46E-03 | 2.35E-05 | 1.38E-02 | 1.62E-04 | 3.30E-02 | 3.45E-04 | 5.06E-03 | 8.50E-05 |
| 3 | 4.48E-03 | 1.42E-04 | 1.58E-02 | 1.34E-04 | 3.75E-02 | 3.92E-04 | 6.55E-03 | 9.15E-05 |
| 4 | 4.76E-03 | 5.65E-05 | 1.67E-02 | 1.18E-04 | 3.99E-02 | 1.25E-04 | 7.21E-03 | 1.10E-04 |
| 8 | 4.15E-03 | - | 1.94E-02 | - | 5.16E-02 | - | 1.21E-03 | - |

Table 3. Average pH during the 8-day for LAWA44 powder altered in varying concentrations of TRIS/HNO3  solution.

| Concentration of TRIS (M) | Average pH |
| --- | --- |
| 0.02 | 8.53 ± 0.04 |
| 0.05 | 8.53 ± 0.06 |
| 0.1 | 8.56 ± 0.04 |
| 0.3 | 8.64 ± 0.06 |

Table 4. ICP-OES elemental concentration data for LAW A44 glass powders altered in 0.1 M TRIS-HNO3 /LAW A44.

Sample	                            0.1 M TRIS/LAW A44

Surface area (m2)	0.02

Density (g m-3)	              2.65

| 0.1 M TRIS/LAW A44 |  | Average elemental concentration across duplicates |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Temperature (°C) | Target pH | Set /measured pH | Time (Hr) | Al (ppm) | B(ppm) | Na (ppm) | Si (ppm) |
| RT | 8.5 | 8.53 | 0.25 | 0.05 ± 0.03 | 0.35 ± 0.04 | 4.83 ± 0.30 | 0.28 ± 0.03 |
|  |  |  | 0.50 | 0.03 ± 0.00 | 0.36 ± 0.01 | 5.73 ± 0.17 | 0.39 ± 0.06 |
|  |  |  | 1.00 | 0.03 ± 0.00 | 0.37 ± 0.01 | 6.21 ± 0.13 | 0.38 ± 0.01 |
|  |  |  | 2.00 | 0.03 ± 0.01 | 0.42 ± 0.01 | 6.89 ± 0.06 | 0.52 ± 0.02 |
|  |  |  | 4.00 | 0.03 ± 0.01 | 0.48 ± 0.01 | 8.01 ± 0.19 | 0.65 ± 0.01 |
|  |  |  | 8.00 | 0.04 ± 0.00 | 0.57 ± 0.01 | 9.16 ± 0.36 | 0.93 ± 0.05 |
|  |  |  | 16.00 | 0.09 ± 0.00 | 0.54 ± 0.02 | 8.48 ± 0.15 | 1.13 ± 0.01 |
|  |  |  | 24.00 | 0.15 ± 0.01 | 0.83 ± 0.01 | 10.04 ± 0.01 | 1.37 ± 0.01 |
|  |  |  | 48.00 | 0.20 ± 0.00 | 0.96 ± 0.02 | 11.70 ± 0.20 | 1.92 ± 0.01 |
|  |  |  | 72.00 | 0.26 ± 0.00 | 1.03 ± 0.01 | 13.28 ± 0.13 | 2.50 ± 0.03 |
|  |  |  | 96.00 | 0.30 ± 0.02 | 1.12 ± 0.01 | 14.21 ± 0.17 | 2.85 ± 0.09 |
|  |  |  | 192.00 | 0.68 ± 0.06 | 1.29 ± 0.02 | 18.62 ± 0.14 | 4.97 ± 0.07 |
| 40 | 8.5 | 8.53 | 0.25 | 0.09 ± 0.01 | 0.37 ± 0.06 | 9.73 ± 0.61 | 0.29 ± 0.04 |
|  |  |  | 0.50 | 0.12 ± 0.02 | 0.37 ± 0.02 | 11.13 ± 0.79 | 0.51 ± 0.15 |
|  |  |  | 1.00 | 0.11 ± 0.00 | 0.41 ± 0.00 | 13.17 ± 0.13 | 0.63 ± 0.02 |
|  |  |  | 2.00 | 0.14 ± 0.02 | 0.44 ± 0.02 | 13.46 ± 0.17 | 0.86 ± 0.10 |
|  |  |  | 4.00 | 0.18 ± 0.00 | 0.51 ± 0.01 | 14.99 ± 0.11 | 1.27 ± 0.17 |
|  |  |  | 8.00 | 0.22 ± 0.01 | 0.60 ± 0.00 | 16.57 ± 0.11 | 1.55 ± 0.02 |
|  |  |  | 16.00 | 0.37 ± 0.01 | 0.87 ± 0.03 | 22.52 ± 0.57 | 2.86 ± 0.13 |
|  |  |  | 24.00 | 0.41 ± 0.00 | 1.25 ± 0.00 | 27.61 ± 0.08 | 3.69 ± 0.18 |
|  |  |  | 48.00 | 0.57 ± 0.04 | 1.62 ± 0.00 | 32.12 ± 0.23 | 5.21 ± 0.04 |
|  |  |  | 72.00 | 0.65 ± 0.00 | 1.85 ± 0.00 | 35.14 ± 0.06 | 6.05 ± 0.05 |
|  |  |  | 96.00 | 0.76 ± 0.06 | 2.16 ± 0.013 | 38.79 ± 1.69 | 7.42 ± 0.55 |
|  |  |  | 192.00 | 1.04 ± 0.04 | 2.84 ± 0.14 | 46.90 ± 2.02 | 10.26 ± 0.55 |
| 60 | 8.5 | 8.52 | 0.25 | 0.11 ± 0.01 | 0.55 ± 0.05 | 13.78 ± 0.14 | 0.67 ± 0.02 |
|  |  |  | 0.50 | 0.15 ± 0.00 | 0.73 ± 0.02 | 17.95 ±0.06 | 1.14 ± 0.01 |
|  |  |  | 1.00 | 0.20 ± 0.02 | 0.88 ± 0.02 | 20.81 ± 0.23 | 1.60 ± 0.07 |
|  |  |  | 2.00 | 0.47 ± 0.08 | 1.41 ± 0.03 | 28.40 ± 0.53 | 3.59 ± 0.50 |
|  |  |  | 4.00 | 0.42 ± 0.01 | 1.55 ± 0.01 | 30.77 ± 0.05 | 3.58 ± 0.04 |
|  |  |  | 8.00 | 0.61 ± 0.01 | 2.05 ± 0.01 | 37.69 ± 0.05 | 5.03 ± 0.02 |
|  |  |  | 16.00 | 0.81 ± 0.01 | 2.82 ± 0.03 | 46.92 ± 0.56 | 6.96 ± 0.10 |
|  |  |  | 24.00 | 0.79 ± 0.01 | 3.48 ± 0.08 | 52.74 ± 0.62 | 7.30 ± 0.07 |
|  |  |  | 48.00 | 1.04 ± 0.04 | 5.26 ± 0.30 | 66.01 ± 3.50 | 10.43 ± 0.40 |
|  |  |  | 72.00 | 1.09 ± 0.01 | 6.12 ± 0.15 | 68.58 ± 0.82 | 11.51 ± 0.08 |
|  |  |  | 96.00 | 1.18 ± 0.03 | 7.01 ± 0.12 | 74.22 ± 0.86 | 12.75 ± 0.35 |
|  |  |  | 192.00 | 1.28 ± 0.05 | 11.66 ± 1.38 | 100.52 ± 7.75 | 16.96 ± 1.64 |

| 0.1 M TRIS/LAW A44 |  | Average elemental concentration across duplicates |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Temperature (°C) | Target pH | Set/ measured pH | Time (Hr) | Al (ppm) | B(ppm) | Na (ppm) | Si (ppm) |
| RT | 9.5 | 9.52 | 0.25 | 0.12 ± 0.04 | 0.26 ± 0.07 | 5.66 ± 0.01 | 0.22 ± 0.04 |
|  |  |  | 0.50 | 0.10 ± 0.00 | 0.21 ± 0.01 | 6.05 ± 0.08 | 0.24 ± 0.01 |
|  |  |  | 1.00 | 0.12 ± 0.00 | 0.24 ± 0.01 | 6.80 ± 0.32 | 0.42 ± 0.02 |
|  |  |  | 2.00 | 0.13 ± 0.00 | 0.25 ± 0.00 | 7.14 ± 0.11 | 0.45 ± 0.01 |
|  |  |  | 4.00 | 0.15 ± 0.00 | 0.28 ± 0.01 | 7.77 ± 0.47 | 0.65 ± 0.00 |
|  |  |  | 8.00 | 0.15 ± 0.00 | 0.32 ± 0.01 | 8.26 ± 0.14 | 0.83 ± 0.10 |
|  |  |  | 16.00 | 0.23 ± 0.01 | 0.37 ± 0.02 | 8.92 ± 0.14 | 1.35 ± 0.01 |
|  |  |  | 24.00 | 0.31 ± 0.01 | 0.51 ± 0.06 | 9.40 ± 0.17 | 1.73 ± 0.00 |
|  |  |  | 48.00 | 0.44 ± 0.02 | 0.56 ± 0.03 | 10.70 ± 0.02 | 2.69 ± 0.00 |
|  |  |  | 72.00 | 0.56 ± 0.00 | 0.61 ± 0.01 | 11.57 ± 0.19 | 3.55 ± 0.07 |
|  |  |  | 96.00 | 0.67 ± 0.00 | 0.70 ± 0.01 | 12.28 ± 0.04 | 4.28 ± 0.03 |
|  |  |  | 192.00 | 1.35 ± 0.54 | 1.19 ± 0.39 | 15.44 ± 1.81 | 8.15 ± 3.14 |
| 40 | 9.5 | 9.53 | 0.25 | 0.19 ± 0.00 | 0.37 ± 0.00 | 11.12 ± 0.06 | 0.78 ± 0.02 |
|  |  |  | 0.50 | 0.14 ± 0.00 | 0.35 ± 0.00 | 11.96 ± 0.15 | 0.62 ± 0.01 |
|  |  |  | 1.00 | 0.15 ± 0.01 | 0.37 ± 0.01 | 12.61 ± 0.29 | 0.75 ± 0.05 |
|  |  |  | 2.00 | 0.21 ± 0.01 | 0.44 ± 0.02 | 13.90 ± 0.78 | 1.14 ± 0.07 |
|  |  |  | 4.00 | 0.30 ± 0.00 | 0.52 ± 0.01 | 15.71 ± 0.03 | 1.74 ± 0.06 |
|  |  |  | 8.00 | 0.43 ± 0.02 | 0.61 ± 0.00 | 17.59 ± 0.25 | 2.51 ± 0.02 |
|  |  |  | 16.00 | 0.61 ± 0.02 | 0.80 ± 0.03 | 20.41 ± 0.50 | 3.80 ± 0.04 |
|  |  |  | 24.00 | 0.84 ± 0.02 | 0.87 ± 0.01 | 21.00 ± 0.04 | 5.00 ± 0.03 |
|  |  |  | 48.00 | 1.12 ± 0.09 | 1.16 ± 0.08 | 23.31 ± 1.72 | 6.89 ± 0.62 |
|  |  |  | 72.00 | 1.43 ± 0.02 | 1.46 ± 0.01 | 27.46 ± 0.31 | 9.18 ± 0.12 |
|  |  |  | 96.00 | 1.54 ± 0.08 | 1.55 ± 0.08 | 27.90 ± 1.44 | 9.91 ± 0.55 |
|  |  |  | 192.00 | 2.25 ± 0.05 | 2.30 ± 0.07 | 35.94 ± 0.91 | 14.88 ± 0.47 |
| 60 | 9.5 | 9.52 | 0.25 | 0.11 ± 0.01 | 0.55 ± 0.05 | 13.78 ± 0.14 | 0.67 ± 0.02 |
|  |  |  | 0.50 | 0.15 ± 0.00 | 0.73 ± 0.00 | 17.95 ± 0.06 | 1.14 ± 0.01 |
|  |  |  | 1.00 | 0.20 ± 0.02 | 0.88 ± 0.02 | 20.81 ± 0.23 | 1.60 ± 0.07 |
|  |  |  | 2.00 | 0.47 ± 0.09 | 1.41 ± 0.03 | 28.40 ± 0.53 | 3.59 ± 0.49 |
|  |  |  | 4.00 | 0.42 ± 0.01 | 1.55 ± 0.01 | 30.77 ± 0.05 | 3.58 ± 0.04 |
|  |  |  | 8.00 | 0.61 ± 0.01 | 2.05 ± 0.01 | 37.69 ± 0.05 | 5.03 ± 0.02 |
|  |  |  | 16.00 | 0.81 ± 0.01 | 2.82 ± 0.03 | 46.92 ± 0.56 | 6.96 ± 0.11 |
|  |  |  | 24.00 | 0.79 ± 0.01 | 3.48 ± 0.08 | 52.74 ± 0.62 | 7.30 ± 0.08 |
|  |  |  | 48.00 | 1.04 ± 0.04 | 5.26 ± 0.30 | 66.01 ± 3.50 | 10.43 ± 0.41 |
|  |  |  | 72.00 | 1.09 ± 0.01 | 6.12 ± 0.15 | 68.58 ± 0.82 | 11.51 ± 0.08 |
|  |  |  | 96.00 | 1.18 ± 0.03 | 7.01 ± 0.12 | 74.22 ± 0.86 | 12.75 ± 0.35 |
|  |  |  | 192.00 | 1.28 ± 0.05 | 11.66 ± 1.38 | 100.52 ± 7.76 | 16.96 ± 1.64 |

| 0.1 M TRIS/LAW A44 |  | Average elemental concentration across duplicates |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Temperature (°C) | Target pH | Set /measured pH | Time (Hr) | Al (ppm) | B(ppm) | Na (ppm) | Si (ppm) |
| RT | 10.5 | 10.51 | 0.25 | 0.10 ± 0.00 | 0.15 ± 0.01 | 5.16 ± 0.32 | 0.24 ± 0.00 |
|  |  |  | 0.50 | 0.10 ± 0.00 | 0.18 ± 0.00 | 5.63 ± 0.32 | 0.30 ± 0.02 |
|  |  |  | 1.00 | 0.12 ± 0.01 | 0.20 ± 0.00 | 5.91 ± 0.23 | 0.38 ± 0.01 |
|  |  |  | 2.00 | 0.14 ± 0.01 | 0.22 ± 0.01 | 6.37 ± 0.00 | 0.54 ± 0.05 |
|  |  |  | 4.00 | 0.17 ± 0.01 | 0.26 ± 0.01 | 6.83 ± 0.07 | 0.83 ± 0.05 |
|  |  |  | 8.00 | 0.24 ± 0.00 | 0.30 ± 0.00 | 7.21 ± 0.17 | 1.22 ± 0.00 |
|  |  |  | 16.00 | 0.32 ± 0.01 | 0.33 ± 0.01 | 7.68 ± 0.20 | 1.64 ± 0.03 |
|  |  |  | 24.00 | 0.42 ± 0.00 | 0.37 ± 0.00 | 7.96 ± 0.03 | 2.18 ± 0.01 |
|  |  |  | 48.00 | 0.69 ± 0.04 | 0.51 ± 0.02 | 9.30 ± 0.18 | 3.68 ± 0.16 |
|  |  |  | 72.00 | 0.84 ± 0.02 | 0.59 ± 0.01 | 9.88 ± 0.03 | 4.55 ± 0.06 |
|  |  |  | 96.00 | 1.00 ± 0.00 | 0.70 ± 0.02 | 10.66 ± 0.22 | 5.47 ± 0.00 |
|  |  |  | 192.00 | 1.37 ± 0.02 | 1.04 ± 0.02 | 13.08 ± 0.41 | 8.24 ± 0.16 |
| 40 | 10.5 | 10.51 | 0.25 | 0.13 ± 0.00 | 0.20 ± 0.00 | 6.15 ± 0.31 | 0.41 ± 0.02 |
|  |  |  | 0.50 | 0.17 ± 0.01 | 0.28 ± 0.01 | 7.46 ± 0.00 | 0.67 ± 0.02 |
|  |  |  | 1.00 | 0.25 ± 0.00 | 0.32 ± 0.00 | 8.12 ± 0.03 | 1.07 ± 0.02 |
|  |  |  | 2.00 | 0.39 ± 0.00 | 0.39 ± 0.00 | 9.18 ± 0.03 | 1.81 ± 0.00 |
|  |  |  | 4.00 | 0.54 ± 0.00 | 0.44 ± 0.00 | 10.02 ± 0.01 | 2.62 ± 0.01 |
|  |  |  | 8.00 | 0.71 ± 0.00 | 0.52 ± 0.00 | 10.88 ± 0.03 | 3.52 ± 0.01 |
|  |  |  | 16.00 | 1.09 ± 0.03 | 0.79 ± 0.00 | 13.72 ± 0.34 | 5.72 0.15 |
|  |  |  | 24.00 | 1.44 ± 0.00 | 0.98 ± 0.04 | 15.26 ± 0.06 | 7.65 ± 0.01 |
|  |  |  | 48.00 | 1.97 ± 0.07 | 1.46 ± 0.06 | 18.07 ± 0.82 | 11.29 ± 0.48 |
|  |  |  | 72.00 | 2.27 ± 0.15 | 1.76 ± 0.06 | 19.51 ± 0.66 | 13.34 ± 0.44 |
|  |  |  | 96.00 | 2.84 ± 0.15 | 2.65 ± 0.17 | 26.66 ± 2.06 | 18.48 ± 1.09 |
|  |  |  | 192.00 | 3.00 ± 0.04 | 2.86 ± 0.06 | 29.48 ± 0.55 | 19.91 ± 0.37 |
| 60 | 10.5 | 10.52 | 0.25 | 0.15 ± 0.00 | 0.32 ± 0.01 | 7.61 ± 0.03 | 0.71 ± 0.02 |
|  |  |  | 0.50 | 0.37 ± 0.01 | 0.46 ± 0.02 | 10.23 ± 0.29 | 1.85 ± 0.06 |
|  |  |  | 1.00 | 0.39 ± 0.02 | 0.43 ± 0.01 | 6.72 ± 0.25 | 1.94 ± 0.03 |
|  |  |  | 2.00 | 0.96 ± 0.01 | 0.79 ± 0.01 | 14.58 ± 0.04 | 5.06 ± 0.03 |
|  |  |  | 4.00 | 1.34 ± 0.02 | 1.09 ± 0.04 | 16.87 ± 0.28 | 7.37 ± 0.15 |
|  |  |  | 8.00 | 1.96 ± 0.02 | 1.74 ± 0.0 | 21.06 ± 0.23 | 11.53 ± 0.17 |
|  |  |  | 16.00 | 2.47 ± 0.00 | 2.48 ± 0.01 | 26.57 ± 0.06 | 15.58 ± 0.01 |
|  |  |  | 24.00 | 2.57 ± 0.01 | 2.66 ± 0.02 | 28.28 ± 0.20 | 16.45 ± 0.02 |
|  |  |  | 48.00 | 2.62 ± 0.05 | 3.65 ± 0.25 | 39.48 ± 3.08 | 20.01 ± 0.43 |
|  |  |  | 72.00 | 2.16 ± 0.02 | 4.35 ± 0.12 | 46.66 ± 0.82 | 19.78 ± 0.07 |
|  |  |  | 96.00 | 1.69 ± 0.04 | 5.58 ± 0.16 | 55.48 ± 1.66 | 19.45 ± 0.11 |
|  |  |  | 192.00 | 1.31 ± 0.04 | 8.95 ± 0.03 | 72.35 ± 1.30 | 18.94 ± 0.22 |

Table 5: Normalised mass loss (g m-2) for Al, B, Na and Si from LAWA44 powder altered in 0.1 M TRIS/HNO3  solution at a target pH of 8.5 and temperatures of RT, 40 oC and 60 oC.

|  | Average normalised mass loss (g m-2) of elements from LAW A44 in 0.1 M TRIS buffer at target pH 8.5 and RT |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Time (Days) | Al | S.D | B | S.D | Na | S.D | Si | S.D |
| 0.25 | 6.98E-04 | 3.45E-04 | 5.86E-03 | 5.24E-04 | 1.51E-02 | 6.60E-04 | 7.18E-04 | 5.50E-05 |
| 0.50 | 5.08E-04 | 1.69E-05 | 6.07E-03 | 7.10E-05 | 1.80E-02 | 3.73E-04 | 1.01E-03 | 1.03E-04 |
| 1.00 | 3.89E-04 | 3.74E-05 | 6.24E-03 | 1.08E-04 | 1.95E-02 | 2.92E-04 | 9.80E-04 | 2.43E-05 |
| 2.00 | 4.14E-04 | 1.69E-05 | 7.08E-03 | 6.02E-05 | 2.16E-02 | 1.32E-04 | 1.33E-03 | 3.80E-05 |
| 4.00 | 4.39E-04 | 9.17E-05 | 8.06E-03 | 8.77E-05 | 2.51E-02 | 4.27E-04 | 1.68E-03 | 2.50E-05 |
| 8.00 | 6.39E-04 | 1.28E-04 | 9.51E-03 | 1.50E-04 | 2.87E-02 | 7.89E-04 | 2.41E-03 | 8.62E-05 |
| 16.00 | 1.27E-03 | 5.87E-06 | 9.04E-03 | 1.82E-04 | 2.66E-02 | 3.42E-04 | 2.90E-03 | 1.67E-05 |
| 24.00 | 2.18E-03 | 1.31E-04 | 1.38E-02 | 1.01E-04 | 3.15E-02 | 1.57E-05 | 3.54E-03 | 2.32E-05 |
| 48.00 | 2.91E-03 | 3.74E-05 | 1.60E-02 | 1.75E-04 | 3.67E-02 | 4.39E-04 | 4.94E-03 | 1.03E-05 |
| 72.00 | 3.83E-03 | 4.18E-05 | 1.72E-02 | 8.36E-05 | 4.16E-02 | 2.98E-04 | 6.45E-03 | 4.64E-05 |
| 96.00 | 4.41E-03 | 1.67E-04 | 1.87E-02 | 8.36E-05 | 4.46E-02 | 3.76E-04 | 7.33E-03 | 1.65E-04 |
| 192.00 | 1.00E-02 | 5.81E-04 | 2.15E-02 | 2.01E-04 | 5.84E-02 | 3.14E-04 | 1.28E-02 | 1.35E-04 |
|  | Average normalised mass loss (g m-2) of elements from LAW A44 in 0.1 M TRIS buffer at target pH 8.5 at 40 oC |  |  |  |  |  |  |  |
| 0.25 | 1.39E-03 | 1.20E-04 | 6.12E-03 | 7.63E-04 | 3.05E-02 | 1.36E-03 | 7.47E-04 | 6.52E-05 |
| 0.50 | 1.75E-03 | 1.70E-04 | 6.20E-03 | 2.64E-04 | 3.49E-02 | 1.76E-03 | 1.32E-03 | 2.70E-04 |
| 1.00 | 1.64E-03 | 2.20E-06 | 6.93E-03 | 3.84E-05 | 4.13E-02 | 2.82E-04 | 1.62E-03 | 2.74E-05 |
| 2.00 | 2.09E-03 | 2.16E-04 | 7.35E-03 | 2.36E-04 | 4.22E-02 | 3.76E-04 | 2.21E-03 | 1.90E-04 |
| 4.00 | 2.68E-03 | 2.76E-04 | 8.57E-03 | 1.53E-04 | 4.70E-02 | 2.51E-04 | 3.26E-03 | 3.10E-04 |
| 8.00 | 3.23E-03 | 9.98E-05 | 9.94E-03 | 4.01E-05 | 5.20E-02 | 2.51E-04 | 4.00E-03 | 4.25E-05 |
| 16.00 | 5.47E-03 | 1.51E-04 | 1.46E-02 | 3.59E-04 | 7.06E-02 | 1.25E-03 | 7.36E-03 | 2.38E-04 |
| 24.00 | 6.01E-03 | 3.59E-05 | 2.09E-02 | 0.00E+00 | 8.66E-02 | 1.88E-04 | 9.51E-03 | 5.80E-05 |
| 48.00 | 8.36E-03 | 3.76E-04 | 2.71E-02 | 5.85E-05 | 1.01E-01 | 5.18E-04 | 1.34E-02 | 3.35E-04 |
| 72.00 | 9.49E-03 | 2.35E-05 | 3.10E-02 | 2.51E-05 | 1.10E-01 | 1.41E-04 | 1.56E-02 | 9.02E-05 |
| 96.00 | 1.11E-02 | 5.71E-04 | 3.62E-02 | 1.56E-03 | 1.22E-01 | 3.75E-03 | 1.91E-02 | 1.01E-03 |
| 192.00 | 1.52E-02 | 4.55E-04 | 4.75E-02 | 1.65E-03 | 1.47E-01 | 4.49E-03 | 2.64E-02 | 1.01E-03 |
|  | Average normalised mass loss (g m-2) of elements from LAW A44 in 0.1 M TRIS buffer at target pH 8.5 at 60 oC |  |  |  |  |  |  |  |
| 0.25 | 1.61E-03 | 1.17E-04 | 9.13E-03 | 5.41E-04 | 4.32E-02 | 3.14E-04 | 1.73E-03 | 4.53E-05 |
| 0.50 | 2.14E-03 | 1.76E-05 | 1.21E-02 | 2.09E-05 | 5.63E-02 | 1.41E-04 | 2.93E-03 | 1.03E-05 |
| 1.00 | 2.94E-03 | 2.00E-04 | 1.47E-02 | 2.88E-04 | 6.53E-02 | 5.18E-04 | 4.12E-03 | 1.28E-04 |
| 2.00 | 6.90E-03 | 9.00E-04 | 2.36E-02 | 3.34E-04 | 8.91E-02 | 1.18E-03 | 9.24E-03 | 8.90E-04 |
| 4.00 | 6.23E-03 | 6.53E-05 | 2.59E-02 | 7.52E-05 | 9.65E-02 | 1.10E-04 | 9.23E-03 | 7.99E-05 |
| 8.00 | 9.00E-03 | 1.24E-04 | 3.42E-02 | 6.68E-05 | 1.18E-01 | 1.10E-04 | 1.29E-02 | 3.61E-05 |
| 16.00 | 1.19E-02 | 6.31E-05 | 4.71E-02 | 2.92E-04 | 1.47E-01 | 1.24E-03 | 1.79E-02 | 1.97E-04 |
| 24.00 | 1.15E-02 | 9.98E-05 | 5.82E-02 | 8.94E-04 | 1.65E-01 | 1.38E-03 | 1.88E-02 | 1.38E-04 |
| 48.00 | 1.53E-02 | 3.67E-04 | 8.79E-02 | 3.60E-03 | 2.07E-01 | 7.76E-03 | 2.69E-02 | 7.47E-04 |
| 72.00 | 1.60E-02 | 5.87E-05 | 1.02E-01 | 1.76E-03 | 2.15E-01 | 1.82E-03 | 2.97E-02 | 1.55E-04 |
| 96.00 | 1.73E-02 | 2.86E-04 | 1.17E-01 | 1.40E-03 | 2.33E-01 | 1.91E-03 | 3.29E-02 | 6.44E-04 |
| 192.00 | 1.87E-02 | 4.99E-04 | 1.95E-01 | 1.63E-02 | 3.15E-01 | 1.72E-02 | 4.37E-02 | 2.99E-03 |

Table 6: Normalised mass loss (g m-2) for Al, B, Na and Si from LAWA44 powder altered in 0.1 M TRIS/HNO3  solution at a target pH of 9.5 and temperatures of RT, 40 oC and 60 oC.

|  | Average normalised mass loss (g m-2) of elements from LAW A44 in 0.1 M TRIS buffer at target pH 9.5 and RT |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Time (Days) | Al | S.D | B | S.D | Na | S.D | Si | S.D |
| 0.25 | 1.74E-03 | 3.65E-04 | 4.32E-03 | 8.01E-04 | 1.77E-02 | 1.10E-05 | 5.65E-04 | 7.36E-05 |
| 0.50 | 1.46E-03 | 1.32E-05 | 3.51E-03 | 7.94E-05 | 1.90E-02 | 1.74E-04 | 6.31E-04 | 1.52E-05 |
| 1.00 | 1.82E-03 | 2.42E-05 | 4.08E-03 | 8.36E-05 | 2.13E-02 | 7.01E-04 | 1.09E-03 | 4.46E-05 |
| 2.00 | 1.90E-03 | 9.54E-06 | 4.15E-03 | 8.36E-07 | 2.24E-02 | 2.57E-04 | 1.15E-03 | 9.02E-06 |
| 4.00 | 2.19E-03 | 2.05E-05 | 4.69E-03 | 1.61E-04 | 2.44E-02 | 1.06E-03 | 1.67E-03 | 2.62E-05 |
| 8.00 | 2.16E-03 | 4.69E-05 | 5.28E-03 | 1.40E-04 | 2.59E-02 | 3.03E-04 | 2.15E-03 | 3.61E-06 |
| 16.00 | 3.44E-03 | 1.40E-04 | 6.12E-03 | 1.77E-04 | 2.80E-02 | 3.11E-04 | 3.49E-03 | 1.83E-04 |
| 24.00 | 4.60E-03 | 1.14E-04 | 8.48E-03 | 7.00E-04 | 2.95E-02 | 3.75E-04 | 4.46E-03 | 1.67E-05 |
| 48.00 | 6.52E-03 | 2.19E-04 | 9.28E-03 | 3.84E-04 | 3.36E-02 | 6.27E-05 | 6.94E-03 | 0.00E+00 |
| 72.00 | 8.17E-03 | 4.18E-05 | 1.02E-02 | 1.04E-04 | 3.63E-02 | 4.23E-04 | 9.14E-03 | 1.28E-04 |
| 96.00 | 9.85E-03 | 7.85E-05 | 1.16E-02 | 1.08E-04 | 3.85E-02 | 7.84E-05 | 1.10E-02 | 5.93E-05 |
| 192.00 | 1.98E-02 | 5.65E-03 | 1.98E-02 | 4.58E-03 | 4.84E-02 | 4.03E-03 | 2.10E-02 | 5.72E-03 |
|  | Average normalised mass loss (g m-2) of elements from LAW A44 in 0.1 M TRIS buffer at target pH 9.5 at 40 oC |  |  |  |  |  |  |  |
| 0.25 | 2.86E-03 | 3.96E-05 | 6.16E-03 | 4.43E-05 | 3.49E-02 | 1.41E-04 | 2.01E-03 | 3.32E-05 |
| 0.50 | 2.09E-03 | 4.55E-05 | 5.88E-03 | 1.84E-05 | 3.75E-02 | 3.29E-04 | 1.61E-03 | 1.34E-05 |
| 1.00 | 2.22E-03 | 8.73E-05 | 6.24E-03 | 1.71E-04 | 3.95E-02 | 6.43E-04 | 1.93E-03 | 8.35E-05 |
| 2.00 | 3.08E-03 | 1.18E-04 | 7.31E-03 | 1.92E-04 | 4.36E-02 | 1.73E-03 | 2.94E-03 | 1.19E-04 |
| 4.00 | 4.43E-03 | 1.76E-05 | 8.65E-03 | 8.19E-05 | 4.93E-02 | 6.27E-05 | 4.49E-03 | 3.99E-05 |
| 8.00 | 6.27E-03 | 1.91E-05 | 1.01E-02 | 4.85E-05 | 5.52E-02 | 5.65E-04 | 6.46E-03 | 7.73E-05 |
| 16.00 | 9.01E-03 | 2.45E-04 | 1.34E-02 | 3.33E-04 | 6.40E-02 | 1.11E-03 | 9.80E-03 | 4.02E-04 |
| 24.00 | 1.24E-02 | 1.89E-04 | 1.46E-02 | 1.21E-04 | 6.59E-02 | 9.41E-05 | 1.29E-02 | 6.18E-05 |
| 48.00 | 1.65E-02 | 9.46E-04 | 1.95E-02 | 8.94E-04 | 7.31E-02 | 3.81E-03 | 1.78E-02 | 1.13E-03 |
| 72.00 | 2.10E-02 | 1.83E-04 | 2.43E-02 | 1.67E-04 | 8.61E-02 | 6.90E-04 | 2.37E-02 | 2.20E-04 |
| 96.00 | 2.27E-02 | 7.99E-04 | 2.60E-02 | 9.11E-04 | 8.75E-02 | 3.20E-03 | 2.55E-02 | 9.98E-04 |
| 192.00 | 3.30E-02 | 4.77E-04 | 3.85E-02 | 8.02E-04 | 1.13E-01 | 2.02E-03 | 3.83E-02 | 8.50E-04 |
|  | Average normalised mass loss (g m-2) of elements from LAW A44 in 0.1 M TRIS buffer at target pH 9.5 at 60 oC |  |  |  |  |  |  |  |
| 0.25 | 1.76E-03 | 1.17E-04 | 6.46E-03 | 1.53E-04 | 2.98E-02 | 1.32E-04 | 1.70E-03 | 1.12E-04 |
| 0.50 | 3.40E-03 | 0.00E-05 | 8.74E-03 | 4.18E-05 | 3.88E-02 | 0.00E-04 | 3.35E-03 | 1.42E-05 |
| 1.00 | 4.15E-03 | 3.22E-05 | 7.60E-03 | 6.43E-05 | 2.46E-02 | 4.17E-04 | 3.83E-03 | 4.12E-05 |
| 2.00 | 9.24E-03 | 1.74E-04 | 1.52E-02 | 7.10E-05 | 5.80E-02 | 1.73E-04 | 9.93E-03 | 1.02E-04 |
| 4.00 | 1.07E-03 | 3.67E-05 | 1.69E-02 | 1.25E-04 | 6.38E-02 | 1.25E-04 | 1.20E-02 | 6.82E-05 |
| 8.00 | 1.51E-03 | 2.12E-04 | 2.33E-02 | 1.50E-05 | 7.72E-01 | 1.41E-04 | 1.75E-02 | 2.47E-05 |
| 16.00 | 2.05E-02 | 1.32E-05 | 3.31E-02 | 3.67E-04 | 9.64E-01 | 2.98E-04 | 2.52E-02 | 1.06E-04 |
| 24.00 | 2.04E-02 | 7.33E-06 | 3.61E-02 | 4.18E-04 | 1.07E-01 | 6.43E-04 | 2.58E-02 | 1.06E-04 |
| 48.00 | 2.67E-02 | 8.80E-05 | 5.00E-02 | 1.00E-04 | 1.33E-01 | 7.68E-04 | 3.51E-02 | 5.15E-04 |
| 72.00 | 3.04E-02 | 0.00E-05 | 5.87E-02 | 6.68E-04 | 1.47E-01 | 1.36E-03 | 4.10E-02 | 1.54E-04 |
| 96.00 | 2.66E-02 | 3.01E-04 | 6.89E-02 | 3.09E-04 | 1.64E-01 | 6.74E-04 | 4.23E-02 | 2.45E-04 |
| 192.00 | 2.01E-02 | 7.33E-04 | 0.14E-01 | 6.09E-03 | 2.39E-01 | 9.00E-03 | 4.45E-02 | 8.37E-04 |

Table 7: Normalised mass loss (g m-2) for Al, B, Na and Si from LAWA44 powder altered in 0.1 M TRIS/HNO3  solution at a target pH of 9.5 and temperatures of RT, 40 oC and 60 oC

|  | Average normalised mass loss (g m-2) of elements from LAW A44 in 0.1 M TRIS buffer at target pH 10.5 and RT |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Time (Days) | Al | S.D | B | S.D | Na | S.D | Si | S.D |
| 0.25 | 1.41E-03 | 3.81E-05 | 2.53E-03 | 6.27E-05 | 1.62E-02 | 7.14E-04 | 6.06E-04 | 1.29E-07 |
| 0.50 | 1.53E-03 | 9.54E-06 | 2.93E-03 | 2.42E-05 | 1.77E-02 | 6.92E-04 | 7.83E-04 | 4.33E-05 |
| 1.00 | 1.73E-03 | 8.73E-05 | 3.27E-03 | 4.93E-05 | 1.85E-02 | 5.03E-04 | 9.88E-04 | 2.27E-05 |
| 2.00 | 1.98E-03 | 5.28E-05 | 3.71E-03 | 7.35E-05 | 2.00E-02 | 3.14E-06 | 1.38E-03 | 8.85E-05 |
| 4.00 | 2.54E-03 | 9.32E-05 | 4.42E-03 | 8.36E-05 | 2.14E-02 | 1.44E-04 | 2.15E-03 | 9.73E-05 |
| 8.00 | 3.49E-03 | 7.33E-06 | 4.98E-03 | 3.76E-05 | 2.26E-02 | 3.70E-04 | 3.16E-03 | 3.86E-06 |
| 16.00 | 4.63E-03 | 5.79E-05 | 5.53E-03 | 1.73E-04 | 2.41E-02 | 4.53E-04 | 4.22E-03 | 4.64E-05 |
| 24.00 | 6.22E-03 | 3.37E-05 | 6.26E-03 | 5.51E-05 | 2.50E-02 | 5.96E-05 | 5.62E-03 | 1.80E-05 |
| 48.00 | 1.01E-02 | 4.09E-04 | 8.50E-03 | 2.90E-04 | 2.92E-02 | 3.92E-04 | 9.49E-03 | 2.99E-04 |
| 72.00 | 1.23E-02 | 1.88E-04 | 9.88E-03 | 6.93E-05 | 3.10E-02 | 5.80E-05 | 1.17E-02 | 1.15E-04 |
| 96.00 | 1.46E-02 | 2.05E-05 | 1.16E-02 | 1.79E-04 | 3.34E-02 | 4.86E-04 | 1.41E-02 | 9.02E-06 |
| 192.00 | 2.01E-02 | 1.76E-04 | 1.74E-02 | 2.84E-04 | 4.10E-02 | 9.10E-04 | 2.12E-02 | 2.86E-04 |
|  | Average normalised mass loss (g m-2) of elements from LAW A44 in 0.1 M TRIS buffer at target pH 10.5 at 40 oC |  |  |  |  |  |  |  |
| 0.25 | 1.96E-03 | 2.79E-05 | 3.28E-03 | 2.92E-05 | 1.93E-02 | 6.98E-04 | 1.04E-03 | 2.92E-05 |
| 0.50 | 2.57E-03 | 1.42E-04 | 4.61E-03 | 8.86E-05 | 2.34E-02 | 9.41E-06 | 1.73E-03 | 2.80E-05 |
| 1.00 | 3.64E-03 | 4.40E-06 | 5.34E-03 | 2.84E-05 | 2.55E-02 | 8.47E-05 | 2.77E-03 | 4.12E-05 |
| 2.00 | 5.71E-03 | 1.17E-05 | 6.46E-03 | 2.01E-05 | 2.88E-02 | 7.68E-05 | 4.66E-03 | 7.73E-06 |
| 4.00 | 7.94E-03 | 1.54E-05 | 7.41E-03 | 5.18E-05 | 3.14E-02 | 1.57E-05 | 6.75E-03 | 2.45E-05 |
| 8.00 | 1.05E-02 | 4.33E-05 | 8.65E-03 | 2.84E-05 | 3.41E-02 | 6.27E-05 | 9.07E-03 | 1.55E-05 |
| 16.00 | 1.59E-02 | 3.15E-04 | 1.32E-02 | 4.90E-04 | 4.30E-02 | 7.53E-04 | 1.48E-02 | 2.74E-04 |
| 24.00 | 2.11E-02 | 3.67E-05 | 1.64E-02 | 3.76E-05 | 4.78E-02 | 1.41E-04 | 1.97E-02 | 9.02E-06 |
| 48.00 | 2.89E-02 | 7.41E-04 | 2.44E-02 | 7.35E-04 | 5.67E-02 | 1.82E-03 | 2.91E-02 | 8.76E-04 |
| 72.00 | 3.33E-02 | 7.41E-04 | 2.95E-02 | 7.44E-04 | 6.12E-02 | 1.46E-03 | 3.44E-02 | 8.12E-04 |
| 96.00 | 4.40E-02 | 1.53E-03 | 4.79E-02 | 1.96E-03 | 9.25E-02 | 4.56E-03 | 5.13E-02 | 1.98E-03 |
| 192.00 | 4.16E-02 | 3.74E-04 | 4.43E-02 | 6.60E-04 | 8.36E-02 | 1.22E-03 | 4.76E-02 | 6.70E-04 |
|  | Average normalised mass loss (g m-2) of elements from LAW A44 in 0.1 M TRIS buffer at target pH 10.5 at 60 oC |  |  |  |  |  |  |  |
| 0.25 | 2.19E-03 | 3.81E-05 | 5.40E-03 | 1.01E-04 | 2.39E-02 | 7.21E-05 | 1.83E-03 | 2.99E-05 |
| 0.50 | 5.47E-03 | 7.77E-05 | 7.68E-03 | 1.90E-04 | 3.21E-02 | 6.43E-04 | 4.77E-03 | 1.16E-04 |
| 1.00 | 5.74E-03 | 1.81E-04 | 7.12E-03 | 1.57E-04 | 2.11E-02 | 5.54E-04 | 5.00E-03 | 5.93E-05 |
| 2.00 | 1.41E-02 | 7.48E-05 | 1.31E-02 | 1.20E-04 | 4.57E-02 | 7.84E-05 | 1.30E-02 | 5.28E-05 |
| 4.00 | 1.96E-02 | 2.27E-04 | 1.82E-02 | 4.34E-04 | 5.29E-02 | 6.12E-04 | 1.90E-02 | 2.73E-04 |
| 8.00 | 2.87E-02 | 2.49E-04 | 2.91E-02 | 1.34E-04 | 6.60E-02 | 5.18E-04 | 2.97E-02 | 3.09E-04 |
| 16.00 | 3.62E-02 | 0.00E+00 | 4.14E-02 | 7.52E-05 | 8.33E-02 | 1.25E-04 | 4.01E-02 | 1.29E-05 |
| 24.00 | 3.77E-02 | 1.47E-04 | 4.44E-02 | 2.01E-04 | 8.87E-02 | 4.39E-04 | 4.24E-02 | 3.86E-05 |
| 48.00 | 3.84E-02 | 5.13E-04 | 6.11E-02 | 2.90E-03 | 1.24E-01 | 6.84E-03 | 5.15E-02 | 7.86E-04 |
| 72.00 | 3.17E-02 | 2.49E-04 | 7.27E-02 | 1.38E-03 | 1.46E-01 | 1.82E-03 | 5.10E-02 | 1.29E-04 |
| 96.00 | 2.48E-02 | 4.18E-04 | 9.33E-02 | 1.88E-03 | 1.74E-01 | 3.69E-03 | 5.01E-02 | 1.93E-04 |
| 192.00 | 1.92E-02 | 4.40E-04 | 1.50E-01 | 3.43E-04 | 2.27E-01 | 2.89E-03 | 4.88E-02 | 3.99E-04 |

Table 8. ICP-OES elemental concentration data for LAWA44 powder altered in varying concentrations of NH4Cl/NH3 solution.

|  |  |  | Average elemental concentration across duplicates |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Sample | Temperature (°C) | Set pH | Time (Days) | Al (ppm) | B(ppm) | Na (ppm) | Si (ppm) |
| 0.02 M NH4Cl-NH3 / LAW A44 | RT | 8.58 | 1 | 0.06 - | 0.65 - | 7.45 - | 1.15 - |
|  |  |  | 2 | 0.12 ± 0.01 | 1.52 ± 0.11 | 17.09 ±0.02 | 2.92 ± 0.05 |
|  |  |  | 3 | 0.11 ± 0.01 | 1.66 ± 0.02 | 19.16 ±0.13 | 3.49 ±0.07 |
|  |  |  | 4 | 0.14 ± 0.01 | 1.63 ± 0.07 | 18.00 ± 0.80 | 3.48 0.15 |
|  |  |  | 8 | 0.26 ±0.03 | 2.03 ±0.16 | 23.79 ± 1.54 | 4.93 0.22 |
| 0.05 M NH4Cl-NH3 / LAW A44 | RT | 8.58 | 1 | 0.05 ± 0.01 | 1.13 ± 0.09 | 14.64 ± 0.67 | 2.01 ± 0.08 |
|  |  |  | 2 | 0.05 ± 0.00 | 1.38 ± 0.01 | 17.08 ± 0.34 | 2.56 ± 0.01 |
|  |  |  | 3 | 0.06 ± 0.03 | 1.51 ± 0.01 | 17.43 ± 0.19 | 2.85 ± 0.08 |
|  |  |  | 4 | 0.11 ± 0.01 | 1.70 ± 0.08 | 20.35 ± 1.23 | 3.40 ± 0.20 |
|  |  |  | 8 | 0.25 ± 0.06 | 2.01 ± 0.23 | 23.91 ± 2.44 | 4.53 ± 0.60 |
| 0.1 M NH4Cl-NH3 / LAW A44 | RT | 8.56 | 1 | 0.04 ± 0.01 | 1.13 ± 0.04 | 16.41 ± 0.50 | 1.93 ± 0.06 |
|  |  |  | 2 | 0.04 ± 0.01 | 1.46 ± 0.12 | 18.17 ± 0.03 | 2.52 ± 0.13 |
|  |  |  | 3 | 0.06 ± 0.02 | 1.70 ± 0.05 | 20.58 ± 2.02 | 2.89 ± 0.16 |
|  |  |  | 4 | 0.06 ± 0.00 | 1.70 ± 0.04 | 21.49 ± 0.14 | 3.16 ± 0.02 |
|  |  |  | 8 | 0.09 ± 0.00 | 1.80 ± 0.00 | 22.47 ± 0.38 | 3.42 ± 0.01 |
| 0.3 M NH4Cl-NH3 / LAW A44 | RT | 8.58 | 1 | 0.03 ± 0.01 | 1.30 ± 0.01 | 23.20 ± 0.78 | 2.15 ± 0.06 |
|  |  |  | 2 | 0.05 ± 0.03 | 1.57 ± 0.10 | 21.97 ± 0.69 | 2.45 ± 0.11 |
|  |  |  | 3 | 0.04 ± 0.01 | 1.72 ± 0.00 | 24.35 ± 1.00 | 2.68 ± 0.10 |
|  |  |  | 4 | 0.03 ± 0.01 | 2.12 ± 0.05 | 30.38 ± 0.63 | 3.41 ± 0.11 |
|  |  |  | 8 | 0.04 ± 0.00 | 1.97 ± 0.07 | 28.59 ± 1.10 | 3.16 ± 0.14 |

Table 9: Normalised mass loss (g m-2) for Al, B, Na and Si from LAWA44 powder altered in varying concentrations of NH4Cl/NH3  solution.

|  | Average normalised mass loss (g m-2) of elements from LAW A44 in 0.02 M ammonia buffer |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Time (days) | Al | S.D. | B | S.D. | Na | S.D. | Si | S.D. |
| 1 | 8.41E-04 | - | 1.08E-02 | - | 2.34E-02 | - | 2.95E-03 | - |
| 2 | 1.77E-03 | 6.40E-04 | 2.53E-02 | 1.25E-03 | 5.36E-02 | 4.70E-05 | 7.52E-03 | 9.02E-05 |
| 3 | 1.61E-03 | 6.97E-05 | 2.78E-02 | 1.84E-04 | 6.01E-02 | 2.98E-04 | 8.98E-03 | 1.28E-04 |
| 4 | 2.08E-03 | 8.21E-05 | 2.72E-02 | 8.19E-04 | 5.64E-02 | 1.77E-03 | 8.96E-03 | 2.74E-04 |
| 8 | 3.83E-03 | 3.45E-04 | 3.39E-02 | 1.89E-03 | 7.46E-02 | 3.42E-03 | 1.27E-02 | 3.99E-04 |
|  | Average normalised mass loss (g m-2)of elements from LAW A44 in 0.05 M ammonia buffer |  |  |  |  |  |  |  |
| 1 | 7.28E-04 | 1.36E-04 | 1.89E-02 | 1.04E-03 | 4.59E-02 | 1.49E-03 | 5.18E-03 | 1.43E-04 |
| 2 | 7.80E-04 | 2.93E-05 | 2.30E-02 | 5.85E-05 | 5.36E-02 | 7.53E-04 | 6.61E-03 | 2.58E-05 |
| 3 | 8.39E-04 | 2.61E-04 | 2.52E-02 | 1.17E-04 | 5.47E-02 | 4.23E-04 | 7.35E-03 | 1.55E-04 |
| 4 | 1.57E-03 | 7.04E-05 | 2.85E-02 | 9.86E-04 | 6.38E-02 | 2.73E-03 | 8.77E-03 | 3.62E-04 |
| 8 | 3.61E-03 | 6.20E-04 | 3.36E-02 | 2.76E-03 | 7.50E-02 | 5.43E-03 | 1.17E-02 | 1.10E-03 |
|  | Average normalised mass loss (g m-2) of elements from LAW A44 in 0.1 M ammonia buffer |  |  |  |  |  |  |  |
| 1 | 5.18E-04 | 7.63E-05 | 1.89E-02 | 4.34E-04 | 5.15E-02 | 1.11E-03 | 4.98E-03 | 1.16E-04 |
| 2 | 5.96E-04 | 1.36E-04 | 2.43E-02 | 1.40E-03 | 5.70E-02 | 6.27E-05 | 6.50E-03 | 2.28E-04 |
| 3 | 8.90E-04 | 2.50E-04 | 2.84E-02 | 5.93E-04 | 6.45E-02 | 4.47E-03 | 7.45E-03 | 2.95E-04 |
| 4 | 8.98E-04 | 4.69E-05 | 2.85E-02 | 4.43E-04 | 6.74E-02 | 3.14E-04 | 8.15E-03 | 3.61E-05 |
| 8 | 1.30E-03 | 4.25E-05 | 3.00E-02 | 8.36E-06 | 7.05E-02 | 8.47E-04 | 8.81E-03 | 2.71E-05 |
|  | Average normalised mass loss (g m-2) of elements from LAW A44 in 0.3 M ammonia buffer |  |  |  |  |  |  |  |
| 1 | 5.05E-04 | 6.01E-05 | 2.18E-02 | 1.25E-04 | 7.28E-02 | 1.74E-03 | 5.53E-03 | 1.07E-04 |
| 2 | 7.26E-04 | 3.26E-04 | 2.63E-02 | 1.18E-03 | 6.89E-02 | 1.52E-03 | 6.32E-03 | 1.96E-04 |
| 3 | 6.59E-04 | 5.87E-05 | 2.88E-02 | 4.18E-05 | 7.64E-02 | 2.21E-03 | 6.91E-03 | 1.77E-04 |
| 4 | 5.09E-04 | 7.48E-05 | 3.54E-02 | 5.43E-04 | 9.53E-02 | 1.40E-03 | 8.78E-03 | 2.07E-04 |
| 8 | 5.87E-04 | 7.33E-06 | 3.30E-02 | 8.27E-04 | 8.97E-02 | 2.43E-03 | 8.15E-03 | 2.60E-04 |

Table 10. Average pH during the 8-day for LAWA44 powder altered in varying concentrations of NH3/NH4Cl solution

| Concentration of NH3/NH4Cl | Average pH |
| --- | --- |
| 0.02 | 8.49 ± 0.08 |
| 0.05 | 8.42 ± 0.12 |
| 0.1 | 8.36 ± 0.11 |
| 0.3 | 8.31 ± 0.11 |

Table 11. ICP-OES elemental concentration data for LAWA44 glass powders altered in 0.1 M NH4Cl-NH3/LAW A44.

Sample	                0.1 M NH4Cl-NH3/LAWA44

Surface area (m2)	0.02

Density (g m-3)	                2.65

| 0.1 M NH4Cl-NH3/LAW A44 |  | Average elemental concentration across duplicates |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Temperature (°C) | Target pH | Set/measured pH | Time (Hr) | Al (ppm) | B(ppm) | Na (ppm) | Si (ppm) |
| RT | 8.5 | 8.52 | 0.25 | 0.04 ± 0.00 | 0.46 ± 0.03 | 9.09 ± 0.32 | 0.39 ± 0.03 |
|  |  |  | 0.50 | 0.02 ± 0.00 | 0.39 ± 0.02 | 9.26 ± 0.09 | 0.40 ± 0.02 |
|  |  |  | 1.00 | 0.06 ± 0.05 | 0.42 ± 0.04 | 9.69 ± 0.39 | 0.73 ± 0.35 |
|  |  |  | 2.00 | 0.03 ± 0.01 | 0.44 ± 0.01 | 10.34 ± 0.17 | 0.70 ± 0.00 |
|  |  |  | 4.00 | 0.03 ± 0.00 | 0.49 ± 0.01 | 11.15 ± 0.32 | 0.91 ± 0.03 |
|  |  |  | 8.00 | 0.06 ± 0.00 | 0.57 ± 0.01 | 12.08 ± 0.22 | 1.23 ± 0.03 |
|  |  |  | 16.00 | 0.10 ± 0.00 | 0.64 ± 0.01 | 12.70 ± 0.14 | 1.76 ± 0.01 |
|  |  |  | 24.00 | 0.04 ± 0.01 | 1.13 ± 0.04 | 16.41 ± 0.50 | 1.93 ± 0.06 |
|  |  |  | 48.00 | 0.04 ± 0.01 | 1.46 ± 0.12 | 18.49 ± 0.42 | 2.52 ± 0.03 |
|  |  |  | 72.00 | 0.06 ± 0.02 | 1.70 ± 0.05 | 20.58 ± 2.02 | 2.89 ± 0.16 |
|  |  |  | 96.00 | 0.06 ± 0.00 | 1.70 ± 0.04 | 21.49 ± 0.14 | 3.16 ± 0.02 |
|  |  |  | 192.00 | 0.09 ± 0.00 | 1.80 ± 0.00 | 22.47 ± 0.38 | 3.42 ± 0.01 |
| 40 | 8.5 | 8.54 | 0.25 | 0.03 ± 0.02 | 0.53 ± 0.04 | 9.95 ± 0.30 | 0.57 ± 0.01 |
|  |  |  | 0.50 | 0.03 ± 0.00 | 0.56 ± 0.02 | 11.04 ± 0.13 | 0.78 ± 0.01 |
|  |  |  | 1.00 | 0.03 ± 0.00 | 0.71 ± 0.00 | 12.66 ± 0.06 | 1.20 ± 0.02 |
|  |  |  | 2.00 | 0.06 ± 0.01 | 0.87 ± 0.01 | 14.31 ± 0.16 | 1.68 ± 0.03 |
|  |  |  | 4.00 | 0.08 ± 0.00 | 1.09 ± 0.05 | 16.38 ± 0.14 | 2.35 ± 0.09 |
|  |  |  | 8.00 | 0.16 ± 0.00 | 1.26 ± 0.01 | 17.78 ± 0.16 | 3.33 ± 0.02 |
|  |  |  | 16.00 | 0.21 ± 0.00 | 1.46 ± 0.01 | 19.89 ± 0.18 | 4.05 ± 0.01 |
|  |  |  | 24.00 | 0.42 ± 0.00 | 2.22 ± 0.07 | 27.23 ± 0.07 | 6.17 ± 0.02 |
|  |  |  | 48.00 | 0.53 ± 0.02 | 2.54 ± 1.05 | 28.79 ± 1.05 | 7.05 ± 0.04 |
|  |  |  | 72.00 | 0.94 ± 0.04 | 3.31 ± 0.19 | 36.28 ± 0.19 | 9.96 ± 0.07 |
|  |  |  | 96.00 | 0.98 ± 0.15 | 3.10 ± 0.13 | 35.59 ± 0.13 | 10.20 ± 0.92 |
|  |  |  | 192.00 | 1.81 ± 0.01 | 4.83 ± 0.26 | 48.10 ± 0.26 | 15.94 ± 0.20 |
| 60 | 8.5 | 8.52 | 0.25 | 0.08 ± 0.01 | 0.76 ± 0.01 | 15.30 ± 0.16 | 1.19 ± 0.04 |
|  |  |  | 0.50 | 0.12 ± 0.01 | 1.05 ± 0.01 | 18.27 ± 0.04 | 1.97 ± 0.04 |
|  |  |  | 1.00 | 0.16 ± 0.00 | 1.62 ± 0.02 | 23.35 ± 0.12 | 3.38 ± 0.01 |
|  |  |  | 2.00 | 0.25 ± 0.01 | 2.34 ± 0.01 | 29.10 ± 0.39 | 5.27 ± 0.07 |
|  |  |  | 4.00 | 0.36 ± 0.00 | 3.12 ± 0.05 | 35.69 ± 0.59 | 7.37 ± 0.05 |
|  |  |  | 8.00 | 0.46 ± 0.17 | 3.87 ± 0.18 | 42.48 ± 2.41 | 8.87 ± 0.32 |
|  |  |  | 16.00 | 0.66 ± 0.27 | 5.27 ± 0.03 | 53.96 ± 0.78 | 11.33 ± 0.06 |
|  |  |  | 24.00 | 0.64 ± 0.00 | 5.83 ± 0.00 | 61.30 ± 0.14 | 11.73 ± 0.07 |
|  |  |  | 48.00 | 0.73 ± 0.05 | 7.12 ± 0.05 | 72.35 ± 0.18 | 12.65 ± 0.11 |
|  |  |  | 72.00 | 0.80 ± 0.02 | 8.38 ± 0.02 | 81.61 ± 0.06 | 13.77 ± 0.03 |
|  |  |  | 96.00 | 0.87 ± 0.01 | 9.13 ± 0.22 | 87.73 ± 1.60 | 14.75 ± 0.24 |
|  |  |  | 192.00 | 1.18 ± 0.03 | 12.42 ± 0.01 | 109.10 ± 2.55 | 18.09 ± 0.13 |
| 0.1 M NH4Cl-NH3/LAW A44 |  | Average elemental concentration across duplicates |  |  |  |  |  |  |
| Temperature (°C) | Target pH | Set/ measured pH | Time (Hr) | Al (ppm) | B(ppm) | Na (ppm) | Si (ppm) |  |
| RT | 9.5 | 9.53 | 0.25 | 0.06 ± 0.03 | 0.30 ± 0.02 | 8.49 ± 0.32 | 0.49 ± 0.20 |  |
|  |  |  | 0.50 | 0.05 ± 0.01 | 0.31 ± 0.01 | 9.12 ± 0.08 | 0.48 ± 0.03 |  |
|  |  |  | 1.00 | 0.05 ± 0.00 | 0.32 ± 0.01 | 9.18 ± 0.00 | 0.61 ± 0.00 |  |
|  |  |  | 2.00 | 0.06 ± 0.00 | 0.34 ± 0.00 | 9.26 ± 0.00 | 0.77 ± 0.00 |  |
|  |  |  | 4.00 | 0.09 ± 0.00 | 0.39 ± 0.00 | 9.93 ± 0.15 | 1.10 ± 0.01 |  |
|  |  |  | 8.00 | 0.13 ± 0.01 | 0.46 ± 0.01 | 10.91 ± 0.28 | 1.53 ± 0.01 |  |
|  |  |  | 16.00 | 0.15 ± 0.00 | 0.54 ± 0.20 | 11.73 ± 0.20 | 1.98 ± 0.04 |  |
|  |  |  | 24.00 | 0.19 ± 0.01 | 0.53 ± 0.02 | 10.57 ± 0.42 | 2.11 ± 0.06 |  |
|  |  |  | 48.00 | 0.24 ± 0.00 | 0.66 ± 0.01 | 11.57 ± 0.11 | 2.72 ± 0.01 |  |
|  |  |  | 72.00 | 0.32 ± 0.00 | 0.78 ± 0.02 | 13.04 ± 0.29 | 3.39 ± 0.06 |  |
|  |  |  | 96.00 | 0.37 ± 0.01 | 0.87 ± 0.02 | 13.68 ± 0.11 | 3.82 ± 0.09 |  |
|  |  |  | 192.00 | 0.56 ± 0.00 | 1.11 ± 0.00 | 15.81 ± 0.06 | 5.15 ± 0.06 |  |
| 40 | 9.5 | 9.51 | 0.25 | 0.05 ± 0.01 | 0.35 ± 0.01 | 9.33 ± 0.06 | 0.66 ± 0.01 |  |
|  |  |  | 0.50 | 0.08 ± 0.02 | 0.41 ± 0.02 | 10.25 ± 0.26 | 1.09 ± 0.13 |  |
|  |  |  | 1.00 | 0.12 ± 0.00 | 0.48 ± 0.01 | 10.76 ± 0.01 | 1.44 ± 0.00 |  |
|  |  |  | 2.00 | 0.18 ± 0.01 | 0.57 ± 0.01 | 12.06 ± 0.07 | 2.04 ± 0.00 |  |
|  |  |  | 4.00 | 0.24 ± 0.00 | 0.70 ± 0.00 | 13.44 ± 0.11 | 2.70 ± 0.04 |  |
|  |  |  | 8.00 | 0.30 ± 0.00 | 0.85 ± 0.01 | 14.81 ± 0.01 | 3.38 ± 0.01 |  |
|  |  |  | 16.00 | 0.37 ± 0.00 | 1.07 ± 0.01 | 17.28 ± 0.11 | 4.19 ± 0.05 |  |
|  |  |  | 24.00 | 0.51 ± 0.01 | 1.70 ± 0.00 | 24.21 ± 0.06 | 6.03 ± 0.03 |  |
|  |  |  | 48.00 | 0.73 ± 0.02 | 2.22 ± 0.02 | 29.23 ± 0.08 | 7.89 ± 0.00 |  |
|  |  |  | 72.00 | 0.90 ± 0.03 | 2.56 ± 0.01 | 31.97 ± 0.55 | 9.11 ± 0.05 |  |
|  |  |  | 96.00 | 1.11 ± 0.00 | 3.26 ± 0.51 | 36.75 ± 2.63 | 10.72 ± 0.40 |  |
|  |  |  | 192.00 | 1.98 ± 0.35 | 4.02 ± 0.23 | 43.35 ± 1.85 | 16.02 ± 1.97 |  |
| 60 | 9.5 | 9.54 | 0.25 | 0.10 ± 0.00 | 0.49 ± 0.00 | 11.98 ± 0.06 | 0.87 ± 0.07 |  |
|  |  |  | 0.50 | 0.20 ± 0.01 | 0.72 ± 0.01 | 14.90 ± 0.14 | 2.03 ± 0.02 |  |
|  |  |  | 1.00 | 0.42 ± 0.00 | 1.27 ± 0.02 | 20.58 ± 0.19 | 4.62 ± 0.02 |  |
|  |  |  | 2.00 | 0.51 ± 0.00 | 1.59 ± 0.00 | 24.07 ± 0.24 | 5.87 ± 0.04 |  |
|  |  |  | 4.00 | 0.67 ± 0.01 | 2.19 ± 0.03 | 30.12 ± 0.18 | 7.80 ± 0.08 |  |
|  |  |  | 8.00 | 0.77 ± 0.01 | 2.76 ± 0.11 | 35.76 ± 1.24 | 9.32 ± 0.25 |  |
|  |  |  | 16.00 | 0.97 ± 0.03 | 3.88 ± 0.33 | 46.45 ± 2.91 | 11.69 ± 0.65 |  |
|  |  |  | 24.00 | 0.91 ± 0.02 | 4.70 ± 0.01 | 51.03 ± 0.56 | 12.12 ± 0.16 |  |
|  |  |  | 48.00 | 1.01 ± 0.03 | 5.45 ± 0.04 | 58.78 ±0.26 | 12.91 ± 0.08 |  |
|  |  |  | 72.00 | 1.10 ± 0.00 | 6.21 ± 0.01 | 67.83 ± 2.08 | 14.15 ± 0.27 |  |
|  |  |  | 96.00 | 1.17 ± 0.02 | 6.77 ± 0.15 | 70.80 ± 1.09 | 14.86 ± 0.23 |  |
|  |  |  | 192.00 | 1.46 ± 0.00 | 8.48 ± 0.00 | 87.83 ± 0.00 | 17.78 ± 0.00 |  |
| 0.1 M NH4Cl-NH3/LAW A44 |  | Average elemental concentration across duplicates |  |  |  |  |  |  |
| Temperature (°C) | Target pH | Set/ measured pH | Time (Hr) | Al (ppm) | B(ppm) | Na (ppm) | Si (ppm) |  |
| RT | 10.5 | 10.54 | 0.25 | 0.02 ± 0.00 | 0.20 ± 0.01 | 6.72 ± 0.10 | 0.45 ± 0.02 |  |
|  |  |  | 0.50 | 0.04 ± 0.02 | 0.21 ± 0.01 | 6.81 ± 0.35 | 0.57 ± 0.01 |  |
|  |  |  | 1.00 | 0.05 ± 0.00 | 0.26 ± 0.00 | 7.86 ± 0.09 | 0.92 ± 0.00 |  |
|  |  |  | 2.00 | 0.12 ± 0.02 | 0.35 ± 0.01 | 8.61 ± 0.44 | 1.37 ± 0.18 |  |
|  |  |  | 4.00 | 0.19 ± 0.00 | 0.36 ± 0.08 | 8.55 ± 0.15 | 1.89 ± 0.02 |  |
|  |  |  | 8.00 | 0.29 ± 0.01 | 0.41 ± 0.03 | 9.50 ± 0.21 | 2.56 ± 0.03 |  |
|  |  |  | 16.00 | 0.39 ± 0.04 | 0.53 ± 0.00 | 10.71 ± 0.23 | 3.26 ± 0.04 |  |
|  |  |  | 24.00 | 0.47 ± 0.02 | 0.62 ± 0.00 | 10.80 ± 0.04 | 4.17 ± 0.00 |  |
|  |  |  | 72.00 | 0.65 ± 0.02 | 0.92 ± 3.00 | 13.08 ± 0.14 | 6.05 ± 0.05 |  |
|  |  |  | 96.00 | 0.63 ± 0.11 | 1.04 ± 0.04 | 13.94 ± 0.77 | 6.66 ± 0.02 |  |
|  |  |  | 192.00 | 0.81 ± 0.01 | 1.14 ± 0.04 | 13.51 ± 0.64 | 7.32 ± 0.30 |  |
| 40 | 10.5 | 10.52 | 0.25 | 0.11 ± 0.01 | 0.40 ± 0.06 | 7.59 ± 0.37 | 0.92 ± 0.04 |  |
|  |  |  | 0.50 | 0.16 ± 0.00 | 0.36 ± 0.02 | 8.14 ± 0.08 | 1.32 ± 0.02 |  |
|  |  |  | 1.00 | 0.27 ± 0.00 | 0.42 ± 0.00 | 8.96 ± 0.10 | 2.04 ± 0.02 |  |
|  |  |  | 2.00 | 0.35 ± 0.04 | 0.48 ± 0.04 | 9.33 ± 0.96 | 2.60 ± 0.24 |  |
|  |  |  | 4.00 | 0.38 ± 0.02 | 0.51 ± 0.02 | 8.88 ± 0.30 | 2.92 ± 0.10 |  |
|  |  |  | 8.00 | 0.55 ± 0.11 | 0.70 ± 0.14 | 10.83 ± 0.3 | 4.18 ± 0.74 |  |
|  |  |  | 16.00 | 0.66 ± 0.01 | 0.91 ± 0.01 | 13.08 ± 2.05 | 5.18 ± 0.05 |  |
|  |  |  | 24.00 | 0.70 ± 0.02 | 1.02 ± 0.05 | 13.04 ± 0.65 | 5.74 ± 0.22 |  |
|  |  |  | 48.00 | 0.81 ± 0.19 | 1.34 ± 0.38 | 15.25 ± 3.04 | 6.77 ± 1.38 |  |
|  |  |  | 72.00 | 1.06 ± 0.11 | 1.78 ± 0.21 | 20.93 ± 2.05 | 9.13 ± 0.88 |  |
|  |  |  | 96.00 | 1.41 - | 2.55 - | 29.27 - | 12.68 - |  |
|  |  |  | 192.00 | 1.67 ± 0.13 | 3.40 ± 0.28 | 36.72 ± 2.14 | 16.21 ± 1.34 |  |
| 60 | 10.5 | 10.51 | 0.25 | 0.09 ± 0.01 | 0.41 ± 0.06 | 9.06 ± 0.24 | 0.83 ± 0.04 |  |
|  |  |  | 0.50 | 0.33 ± 0.02 | 0.47 ± 0.04 | 10.27 ± 0.57 | 2.22 ± 0.12 |  |
|  |  |  | 1.00 | 0.65 ± 0.01 | 0.75 ± 0.01 | 12.89 ± 0.14 | 4.64 ± 0.07 |  |
|  |  |  | 2.00 | 0.77 ± 0.00 | 0.95 ± 0.02 | 14.75 ± 0.18 | 5.63 ± 0.03 |  |
|  |  |  | 4.00 | 0.94 ± 0.02 | 1.32 ± 0.02 | 18.48 ± 0.37 | 7.28 ± 0.17 |  |
|  |  |  | 8.00 | 1.06 ± 0.01 | 1.58 ± 0.05 | 20.51 ± 0.10 | 8.41 ± 0.16 |  |
|  |  |  | 16.00 | 1.15 ± 0.01 | 1.92 ± 0.00 | 24.87 ± 0.21 | 9.56 ± 0.07 |  |
|  |  |  | 24.00 | 1.09 ± 0.00 | 2.69 ± 0.09 | 29.82 ± 0.53 | 10.46 ± 0.16 |  |
|  |  |  | 48.00 | 1.20 ± 0.03 | 3.08 ± 0.09 | 34.76 ± 0.54 | 11.73 ± 0.18 |  |
|  |  |  | 72.00 | 1.29 ± 0.02 | 3.44 ± 0.02 | 39.03 ± 0.38 | 12.73 ± 0.06 |  |
|  |  |  | 96.00 | 1.38 ± 0.08 | 3.90 ± 0.25 | 44.30 ± 4.58 | 14.02 ± 1.26 |  |
|  |  |  | 192.00 | 1.60 ± 0.11 | 5.17 ± 1.55 | 56.89 ± 11.49 | 17.42 ± 3.46 |  |

Table 12: Normalised mass loss (g m-2) for Al, B, Na and Si from LAWA44 powder altered in 0.1 M NH4Cl/NH3  solution at target pH 8.5 and temperatures of RT, 40 oC and 60 oC.

|  | Average normalised mass loss of elements from LAW A44 in 0.1 M ammonia buffer at target pH 8.5 and RT |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Time (Days) | Al | S.D | B | S.D | Na | S.D | Si | S.D |
| 0.25 | 5.73E-04 | 2.42E-05 | 7.61E-03 | 3.89E-04 | 2.85E-02 | 7.18E-04 | 1.00E-03 | 5.85E-05 |
| 0.50 | 3.21E-04 | 6.60E-06 | 6.54E-03 | 1.84E-04 | 2.90E-02 | 1.91E-04 | 1.03E-03 | 4.07E-05 |
| 1.00 | 9.41E-04 | 5.55E-04 | 7.07E-03 | 4.85E-04 | 3.04E-02 | 8.58E-04 | 1.87E-03 | 6.33E-04 |
| 2.00 | 4.66E-04 | 7.48E-05 | 7.31E-03 | 1.01E-04 | 3.24E-02 | 3.76E-04 | 1.79E-03 | 2.83E-06 |
| 4.00 | 4.84E-04 | 2.20E-05 | 8.13E-03 | 1.65E-04 | 3.50E-02 | 7.06E-04 | 2.34E-03 | 6.09E-05 |
| 8.00 | 8.09E-04 | 4.33E-05 | 9.52E-03 | 8.94E-05 | 3.79E-02 | 4.86E-04 | 3.18E-03 | 4.77E-05 |
| 16.00 | 1.40E-03 | 7.33E-06 | 1.08E-02 | 6.52E-05 | 3.98E-02 | 3.14E-04 | 4.55E-03 | 1.16E-05 |
| 24.00 | 5.18E-04 | 7.63E-05 | 1.89E-02 | 4.34E-04 | 5.15E-02 | 1.11E-03 | 4.98E-03 | 1.16E-04 |
| 48.00 | 5.96E-04 | 1.36E-04 | 2.43E-02 | 1.40E-03 | 5.80E-02 | 9.25E-04 | 6.50E-03 | 2.28E-04 |
| 72.00 | 8.90E-04 | 2.50E-04 | 2.84E-02 | 5.93E-04 | 6.45E-02 | 4.47E-03 | 7.45E-03 | 2.95E-04 |
| 96.00 | 8.98E-04 | 4.69E-05 | 2.85E-02 | 4.43E-04 | 6.74E-02 | 3.14E-04 | 8.15E-03 | 3.61E-05 |
| 192.00 | 1.30E-03 | 4.25E-05 | 3.00E-02 | 8.36E-06 | 7.05E-02 | 8.47E-04 | 8.81E-03 | 2.71E-05 |
|  | Average normalised mass loss of elements from LAW A44 in 0.1 M ammonia buffer at target pH 8.5 at 40 oC |  |  |  |  |  |  |  |
| 0.25 | 4.06E-04 | 1.69E-04 | 8.90E-03 | 5.26E-04 | 3.12E-02 | 6.56E-04 | 1.46E-03 | 1.42E-05 |
| 0.50 | 4.21E-04 | 1.91E-05 | 9.30E-03 | 2.31E-04 | 3.46E-02 | 2.98E-04 | 2.02E-03 | 9.66E-06 |
| 1.00 | 4.99E-04 | 2.42E-05 | 1.18E-02 | 4.85E-05 | 3.97E-02 | 1.25E-04 | 3.08E-03 | 2.96E-05 |
| 2.00 | 9.01E-04 | 7.63E-05 | 1.46E-02 | 1.41E-04 | 4.49E-02 | 3.61E-04 | 4.33E-03 | 4.90E-05 |
| 4.00 | 1.10E-03 | 9.54E-06 | 1.82E-02 | 5.77E-04 | 5.14E-02 | 3.14E-04 | 6.07E-03 | 1.60E-04 |
| 8.00 | 2.37E-03 | 5.13E-06 | 2.10E-02 | 1.67E-04 | 5.58E-02 | 3.61E-04 | 8.57E-03 | 2.83E-05 |
| 16.00 | 3.13E-03 | 1.03E-05 | 2.44E-02 | 1.34E-04 | 6.24E-02 | 4.08E-04 | 1.04E-02 | 1.55E-05 |
| 24.00 | 6.20E-03 | 1.83E-05 | 3.71E-02 | 1.25E-04 | 8.54E-02 | 1.57E-04 | 1.59E-02 | 3.86E-05 |
| 48.00 | 7.71E-03 | 2.42E-04 | 4.25E-02 | 4.26E-04 | 9.03E-02 | 2.32E-03 | 1.82E-02 | 8.12E-05 |
| 72.00 | 1.37E-02 | 4.48E-04 | 5.53E-02 | 8.36E-06 | 1.14E-01 | 4.23E-04 | 2.57E-02 | 1.29E-04 |
| 96.00 | 1.43E-02 | 1.51E-03 | 5.18E-02 | 1.88E-03 | 1.12E-01 | 2.98E-04 | 2.63E-02 | 1.67E-03 |
| 192.00 | 2.66E-02 | 1.03E-04 | 8.06E-02 | 2.42E-04 | 1.51E-01 | 5.80E-04 | 4.11E-02 | 3.61E-04 |
|  | Average normalised mass loss of elements from LAW A44 in 0.1 M ammonia buffer at target pH 8.5 at 60 oC |  |  |  |  |  |  |  |
| 0.25 | 1.16E-03 | 7.85E-05 | 1.28E-02 | 1.37E-04 | 4.80E-02 | 3.45E-04 | 3.06E-03 | 7.34E-05 |
| 0.50 | 1.73E-03 | 1.36E-04 | 1.76E-02 | 9.19E-05 | 5.73E-02 | 9.41E-05 | 5.09E-03 | 6.96E-05 |
| 1.00 | 2.34E-03 | 1.47E-06 | 2.71E-02 | 2.76E-04 | 7.32E-02 | 2.82E-04 | 8.70E-03 | 2.32E-05 |
| 2.00 | 3.63E-03 | 7.04E-05 | 3.91E-02 | 7.52E-05 | 9.13E-02 | 8.63E-04 | 1.36E-02 | 1.24E-04 |
| 4.00 | 5.33E-03 | 8.07E-06 | 5.22E-02 | 6.60E-04 | 1.12E-01 | 1.30E-03 | 1.90E-02 | 9.92E-05 |
| 8.00 | 6.72E-03 | 5.21E-05 | 6.47E-02 | 2.08E-03 | 1.33E-01 | 5.35E-03 | 2.29E-02 | 5.89E-04 |
| 16.00 | 9.67E-03 | 5.13E-06 | 8.81E-02 | 3.17E-04 | 1.69E-01 | 1.73E-03 | 2.92E-02 | 1.16E-04 |
| 24.00 | 9.38E-03 | 6.16E-05 | 9.74E-02 | 5.01E-05 | 1.92E-01 | 3.14E-04 | 3.02E-02 | 1.29E-04 |
| 48.00 | 1.07E-02 | 7.99E-05 | 1.19E-01 | 5.43E-04 | 2.27E-01 | 3.92E-04 | 3.26E-02 | 2.06E-04 |
| 72.00 | 1.17E-02 | 8.21E-05 | 1.40E-01 | 1.92E-04 | 2.56E-01 | 1.25E-04 | 3.55E-02 | 5.15E-05 |
| 96.00 | 1.28E-02 | 6.01E-05 | 1.53E-01 | 2.62E-03 | 2.75E-01 | 3.54E-03 | 3.80E-02 | 4.38E-04 |
| 192.00 | 1.73E-02 | 3.37E-04 | 2.08E-01 | 1.67E-04 | 3.42E-01 | 5.65E-03 | 4.66E-02 | 2.32E-04 |

Table 13: Normalised mass loss (g m-2) for Al, B, Na and Si from LAWA44 powder altered in 0.1 M NH4Cl/NH3  solution at target pH 9.5 and temperatures of RT, 40 oC and 60 oC.

|  | Average normalised mass loss of elements from LAW A44 in 0.1 M ammonia buffer at target pH 9.5 and RT |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Time (Days) | Al | S.D | B | S.D | Na | S.D | Si | S.D |
| 0.25 | 8.74E-04 | 3.59E-04 | 4.98E-03 | 2.56E-04 | 2.66E-02 | 7.12E-04 | 1.26E-03 | 3.62E-04 |
| 0.50 | 6.73E-04 | 6.53E-05 | 5.13E-03 | 5.93E-05 | 2.86E-02 | 1.74E-04 | 1.25E-03 | 4.78E-05 |
| 1.00 | 6.91E-04 | 1.76E-05 | 5.34E-03 | 1.15E-04 | 2.88E-02 | 4.70E-06 | 1.57E-03 | 1.29E-06 |
| 2.00 | 9.40E-04 | 1.47E-06 | 5.72E-03 | 4.18E-05 | 2.90E-02 | 9.41E-06 | 1.99E-03 | 5.02E-06 |
| 4.00 | 1.29E-03 | 5.57E-05 | 6.46E-03 | 4.93E-05 | 3.11E-02 | 3.22E-04 | 2.85E-03 | 1.93E-05 |
| 8.00 | 1.87E-03 | 2.13E-05 | 7.65E-03 | 6.93E-05 | 3.42E-02 | 6.12E-04 | 3.95E-03 | 1.80E-05 |
| 16.00 | 2.24E-03 | 4.25E-05 | 9.00E-03 | 4.68E-05 | 3.68E-02 | 4.39E-04 | 5.11E-03 | 6.83E-05 |
| 24.00 | 2.74E-03 | 5.50E-05 | 8.80E-03 | 2.00E-04 | 3.31E-02 | 9.25E-04 | 5.44E-03 | 1.11E-04 |
| 48.00 | 3.50E-03 | 1.54E-05 | 1.10E-02 | 1.51E-04 | 3.63E-02 | 2.51E-04 | 7.01E-03 | 1.29E-05 |
| 72.00 | 4.74E-03 | 4.99E-05 | 1.30E-02 | 1.84E-04 | 4.09E-02 | 6.43E-04 | 8.73E-03 | 1.13E-04 |
| 96.00 | 5.46E-03 | 8.51E-05 | 1.45E-02 | 2.35E-04 | 4.29E-02 | 2.51E-04 | 9.85E-03 | 1.69E-04 |
| 192.00 | 8.20E-03 | 7.33E-07 | 1.86E-02 | 8.36E-06 | 4.96E-02 | 1.25E-04 | 1.33E-02 | 1.00E-04 |
|  | Average normalised mass loss of elements from LAW A44 in 0.1 M ammonia buffer at target pH 9.5 at 40 oC |  |  |  |  |  |  |  |
| 0.25 | 7.06E-04 | 8.80E-05 | 5.77E-03 | 1.03E-04 | 2.93E-02 | 1.24E-04 | 1.70E-03 | 1.80E-05 |
| 0.50 | 1.25E-03 | 1.95E-04 | 6.91E-03 | 2.70E-04 | 3.21E-02 | 5.80E-04 | 2.81E-03 | 2.31E-04 |
| 1.00 | 1.79E-03 | 4.55E-05 | 8.04E-03 | 1.16E-04 | 3.38E-02 | 3.14E-05 | 3.72E-03 | 1.29E-06 |
| 2.00 | 2.58E-03 | 1.45E-04 | 9.60E-03 | 1.67E-04 | 3.78E-02 | 1.57E-04 | 5.26E-03 | 3.86E-06 |
| 4.00 | 3.45E-03 | 1.47E-05 | 1.18E-02 | 3.93E-05 | 4.22E-02 | 2.51E-04 | 6.96E-03 | 6.83E-05 |
| 8.00 | 4.47E-03 | 1.17E-05 | 1.42E-02 | 8.61E-05 | 4.65E-02 | 3.14E-05 | 8.70E-03 | 1.03E-05 |
| 16.00 | 5.42E-03 | 3.74E-05 | 1.79E-02 | 1.17E-04 | 5.42E-02 | 2.51E-04 | 1.08E-02 | 9.53E-05 |
| 24.00 | 7.54E-03 | 8.21E-05 | 2.84E-02 | 5.85E-05 | 7.59E-02 | 1.25E-04 | 1.55E-02 | 5.15E-05 |
| 48.00 | 1.07E-02 | 2.38E-04 | 3.72E-02 | 2.34E-04 | 9.17E-02 | 1.88E-04 | 2.03E-02 | 3.86E-06 |
| 72.00 | 1.33E-02 | 2.82E-04 | 4.27E-02 | 1.00E-04 | 1.00E-01 | 1.21E-03 | 2.35E-02 | 8.76E-05 |
| 96.00 | 1.63E-02 | 4.40E-05 | 5.44E-02 | 5.98E-03 | 1.15E-01 | 5.83E-03 | 2.76E-02 | 7.34E-04 |
| 192.00 | 2.90E-02 | 3.65E-03 | 6.72E-02 | 2.67E-03 | 1.36E-01 | 4.11E-03 | 4.13E-02 | 3.59E-03 |
|  | Average normalised mass loss of elements from LAW A44 in 0.1 M ammonia buffer at target pH 9.5 at 60 oC |  |  |  |  |  |  |  |
| 0.25 | 1.50E-03 | 7.33E-06 | 8.13E-03 | 3.84E-05 | 3.76E-02 | 1.41E-04 | 2.24E-03 | 1.19E-04 |
| 0.50 | 2.89E-03 | 1.08E-04 | 1.21E-02 | 7.27E-05 | 4.67E-02 | 3.14E-04 | 5.22E-03 | 3.48E-05 |
| 1.00 | 6.13E-03 | 1.03E-05 | 2.12E-02 | 1.92E-04 | 6.45E-02 | 4.23E-04 | 1.19E-02 | 2.96E-05 |
| 2.00 | 7.55E-03 | 2.35E-05 | 2.66E-02 | 1.67E-05 | 7.55E-02 | 5.49E-04 | 1.51E-02 | 6.44E-05 |
| 4.00 | 9.80E-03 | 8.80E-05 | 3.67E-02 | 3.09E-04 | 9.45E-02 | 3.92E-04 | 2.01E-02 | 1.46E-04 |
| 8.00 | 1.13E-02 | 7.48E-05 | 4.62E-02 | 1.32E-03 | 1.12E-01 | 2.74E-03 | 2.40E-02 | 4.56E-04 |
| 16.00 | 1.42E-02 | 2.99E-04 | 6.48E-02 | 3.87E-03 | 1.46E-01 | 6.46E-03 | 3.01E-02 | 1.19E-03 |
| 24.00 | 1.34E-02 | 1.75E-04 | 7.85E-02 | 1.42E-04 | 1.60E-01 | 1.24E-03 | 3.12E-02 | 2.83E-04 |
| 48.00 | 1.48E-02 | 2.77E-04 | 9.11E-02 | 4.26E-04 | 1.84E-01 | 5.80E-04 | 3.33E-02 | 1.55E-04 |
| 72.00 | 1.61E-02 | 7.33E-06 | 1.04E-01 | 1.75E-04 | 2.13E-01 | 4.61E-03 | 3.64E-02 | 6.83E-04 |
| 96.00 | 1.71E-02 | 1.69E-04 | 1.13E-01 | 1.74E-03 | 2.22E-01 | 2.42E-03 | 3.83E-02 | 2.32E-04 |
| 192.00 | 2.14E-02 | 0.00E+00 | 1.42E-01 | 0.00E+00 | 2.75E-01 | 0.00E+00 | 4.58E-02 | 0.00E+00 |

Table 14: Normalised mass loss (g m-2) for Al, B, Na and Si from LAWA44 powder altered in 0.1 M NH4Cl/NH3  solution at target pH 10.5 and temperatures of RT, 40 oC and 60 oC.

|  | Average normalised mass loss of elements from LAW A44 in 0.1 M ammonia buffer at target pH 10.5 and RT |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Time (Days) | Al | S.D | B | S.D | Na | S.D | Si | S.D |
| 0.25 | 2.67E-04 | 4.40E-05 | 3.41E-03 | 1.27E-04 | 2.11E-02 | 2.23E-04 | 1.15E-03 | 3.16E-05 |
| 0.50 | 5.82E-04 | 1.75E-04 | 3.50E-03 | 1.26E-04 | 2.14E-02 | 7.86E-04 | 1.48E-03 | 2.64E-05 |
| 1.00 | 8.01E-04 | 5.13E-05 | 4.39E-03 | 8.61E-05 | 2.47E-02 | 1.99E-04 | 2.36E-03 | 1.67E-06 |
| 2.00 | 1.72E-03 | 2.69E-04 | 5.82E-03 | 9.88E-04 | 2.70E-02 | 9.82E-04 | 3.54E-03 | 3.30E-04 |
| 4.00 | 2.83E-03 | 3.67E-05 | 6.10E-03 | 3.03E-04 | 2.68E-02 | 3.34E-04 | 4.86E-03 | 3.61E-05 |
| 8.00 | 4.20E-03 | 9.10E-05 | 6.91E-03 | 2.01E-05 | 2.98E-02 | 4.81E-04 | 6.60E-03 | 4.64E-05 |
| 16.00 | 5.67E-03 | 4.65E-04 | 8.87E-03 | 4.60E-05 | 3.36E-02 | 5.18E-04 | 8.39E-03 | 7.09E-05 |
| 24.00 | 6.94E-03 | 1.77E-04 | 1.03E-02 | 8.36E-06 | 3.39E-02 | 9.41E-05 | 1.07E-02 | 2.58E-06 |
| 48.00 | 8.74E-03 | 2.27E-03 | 5.32E-02 | 3.53E-02 | 7.95E-02 | 3.53E-02 | 1.85E-02 | 1.58E-03 |
| 72.00 | 9.52E-03 | 1.94E-04 | 1.53E-02 | 2.42E-05 | 4.10E-02 | 3.29E-04 | 1.56E-02 | 9.28E-05 |
| 96.00 | 9.29E-03 | 1.16E-03 | 1.74E-02 | 5.43E-04 | 4.37E-02 | 1.71E-03 | 1.72E-02 | 3.81E-04 |
| 192.00 | 1.19E-02 | 8.73E-05 | 1.90E-02 | 4.51E-04 | 4.24E-02 | 1.41E-03 | 1.89E-02 | 5.48E-04 |
|  | Average normalised mass loss of elements from LAW A44 in 0.1 M ammonia buffer at target pH 10.5 at 40 oC |  |  |  |  |  |  |  |
| 0.25 | 1.65E-03 | 9.39E-05 | 6.65E-03 | 7.12E-04 | 2.38E-02 | 8.14E-04 | 2.38E-03 | 7.10E-05 |
| 0.50 | 2.39E-03 | 3.67E-05 | 6.06E-03 | 1.90E-04 | 2.55E-02 | 1.87E-04 | 3.40E-03 | 3.61E-05 |
| 1.00 | 3.97E-03 | 2.93E-06 | 7.09E-03 | 1.75E-05 | 2.81E-02 | 2.27E-04 | 5.26E-03 | 2.83E-05 |
| 2.00 | 5.11E-03 | 4.27E-04 | 8.05E-03 | 5.05E-04 | 2.93E-02 | 2.13E-03 | 6.70E-03 | 4.29E-04 |
| 4.00 | 5.54E-03 | 2.20E-04 | 8.58E-03 | 2.52E-04 | 2.78E-02 | 6.62E-04 | 7.53E-03 | 1.88E-04 |
| 8.00 | 8.13E-03 | 1.10E-03 | 1.16E-02 | 1.66E-03 | 3.40E-02 | 4.55E-03 | 1.08E-02 | 1.35E-03 |
| 16.00 | 9.65E-03 | 1.13E-04 | 1.53E-02 | 1.55E-04 | 4.10E-02 | 2.67E-04 | 1.34E-02 | 8.89E-05 |
| 24.00 | 1.02E-02 | 1.80E-04 | 1.70E-02 | 5.61E-04 | 4.09E-02 | 1.44E-03 | 1.48E-02 | 3.98E-04 |
| 48.00 | 1.20E-02 | 1.95E-03 | 2.23E-02 | 4.48E-03 | 4.78E-02 | 6.74E-03 | 1.75E-02 | 2.52E-03 |
| 72.00 | 1.56E-02 | 1.16E-03 | 2.97E-02 | 2.42E-03 | 6.57E-02 | 4.55E-03 | 2.35E-02 | 1.60E-03 |
| 96.00 | 2.07E-02 | 0.00E+00 | 4.25E-02 | 0.00E+00 | 9.18E-02 | 0.00E+00 | 3.27E-02 | 0.00E+00 |
| 192.00 | 2.46E-02 | 1.33E-03 | 5.69E-02 | 3.30E-03 | 1.15E-01 | 4.74E-03 | 4.18E-02 | 2.43E-03 |
|  | Average normalised mass loss of elements from LAW A44 in 0.1 M ammonia buffer at target pH 10.5 at 60 oC |  |  |  |  |  |  |  |
| 0.25 | 1.37E-03 | 1.08E-04 | 6.86E-03 | 6.93E-04 | 2.84E-02 | 5.38E-04 | 2.13E-03 | 6.70E-05 |
| 0.50 | 4.80E-03 | 2.51E-04 | 7.84E-03 | 4.47E-04 | 3.22E-02 | 1.28E-03 | 5.73E-03 | 2.18E-04 |
| 1.00 | 9.57E-03 | 1.86E-04 | 1.25E-02 | 1.70E-04 | 4.04E-02 | 3.14E-04 | 1.20E-02 | 1.34E-04 |
| 2.00 | 1.13E-02 | 4.11E-05 | 1.58E-02 | 1.98E-04 | 4.63E-02 | 4.08E-04 | 1.45E-02 | 5.67E-05 |
| 4.00 | 1.38E-02 | 2.03E-04 | 2.20E-02 | 2.76E-04 | 5.80E-02 | 8.16E-04 | 1.88E-02 | 3.04E-04 |
| 8.00 | 1.56E-02 | 1.32E-04 | 2.64E-02 | 5.51E-04 | 6.43E-02 | 2.21E-03 | 2.17E-02 | 3.00E-04 |
| 16.00 | 1.69E-02 | 1.39E-04 | 3.22E-02 | 8.36E-06 | 7.80E-02 | 4.55E-04 | 2.46E-02 | 1.21E-04 |
| 24.00 | 1.60E-02 | 4.40E-05 | 4.49E-02 | 1.01E-03 | 9.35E-02 | 1.18E-03 | 2.69E-02 | 2.96E-04 |
| 48.00 | 1.76E-02 | 2.64E-04 | 5.15E-02 | 1.08E-03 | 1.09E-01 | 1.21E-03 | 3.02E-02 | 3.35E-04 |
| 72.00 | 1.89E-02 | 1.69E-04 | 5.74E-02 | 2.67E-04 | 1.22E-01 | 8.31E-04 | 3.28E-02 | 1.16E-04 |
| 96.00 | 2.03E-02 | 7.77E-04 | 6.52E-02 | 4.18E-03 | 1.39E-01 | 1.01E-02 | 3.61E-02 | 2.29E-03 |
| 192.00 | 2.35E-02 | 1.14E-03 | 8.64E-02 | 1.83E-02 | 1.78E-01 | 2.55E-02 | 4.49E-02 | 6.30E-03 |

Table 15. Activation energy calculated using linear regression of normalised boron dissolution rates as a function of temperature for LAWA44 at varying pH.

| Timeframe | Target pH | Temperature /⁰C) | Tris buffer | R2 | Ammonia buffer | R2 |
| --- | --- | --- | --- | --- | --- | --- |
|  |  |  | Ea /kJ mol‒1 |  | Ea /kJ mol‒1 |  |
| 15 min to 8 h data | 8.5 | RT | - | - | 57 ± 2 | 0.99 |
|  |  | 40 |  |  |  |  |
|  |  | 60 |  |  |  |  |
|  | 9.5 | RT | 47 ± 5 | 0.98 | 49 ± 7 | 0.95 |
|  |  | 40 |  |  |  |  |
|  |  | 60 |  |  |  |  |
|  | 10.5 | RT | 54 ± 8 | 0.96 | 32 ± 12 | 0.75 |
|  |  | 40 |  |  |  |  |
|  |  | 60 |  |  |  |  |
| 24 h to 96 h data | 8.5 | RT | 47 ± 6 | 0.97 | 33 ± 9 | 0.86 |
|  |  | 40 |  |  |  |  |
|  |  | 60 |  |  |  |  |
|  | 9.5 | RT | 45 ± 5 | 0.99 | 36 ± 10 | 0.84 |
|  |  | 40 |  |  |  |  |
|  |  | 60 |  |  |  |  |
|  | 10.5 | RT | 43 ± 9 | 0.92 | - | - |
|  |  | 40 |  |  |  |  |
|  |  | 60 |  |  |  |  |
| 15 min to 8 d data | 8.5 | RT | 45 ± 8 | 0.94 | 37 ± 3 | 0.99 |
|  |  | 40 |  |  |  |  |
|  |  | 60 |  |  |  |  |
|  | 9.5 | RT | 40 ± 9 | 0.90 | 43 ± 7 | 0.95 |
|  |  | 40 |  |  |  |  |
|  |  | 60 |  |  |  |  |
|  | 10.5 | RT | 44 ± 1 | 0.99 | 31 ± 7 | 0.91 |
|  |  | 40 |  |  |  |  |
|  |  | 60 |  |  |  |  |

Table 16. Composition of LAWA44 glass in oxide wt %.

| Components | Oxide wt% |
| --- | --- |
| Al2O3 | 6.39 |
| B2O3 | 9.56 |
| CaO | 2.21 |
| Cr2O3 | 0.11 |
| Fe2O3 | 7.44 |
| K2O | 0.58 |
| MgO | 1.82 |
| MoO3 | 0.01 |
| Na2O | 21.32 |
| Re2O7 | 0.07 |
| SO3 | 0.11 |
| SiO2 | 41.19 |
| TiO2 | 2.10 |
| ZnO | 3.28 |
| ZrO2 | 3.00 |