Electronic Supporting Information

Magnetic DL-methionine grafted to chitosan by EDTA linker nanomaterial: a highly efficient multifunctional organocatalyst for the synthesis of highly substituted imidazole derivatives under green conditions

Mohammad Dohendou1, Mohammad G. Dekamin1*, Zahra Dehnamaki1, Danial Namaki1 and Suranjana V. Mayani2

1Pharmaceutical and Biologically-Active Compounds Research Laboratory, Department of Chemistry, Iran University of Science and Technology, Tehran 16846-13114, Iran.

2Department of Chemistry, Marwadi University, Rajkot-Morbi Road, P.O. Gauridad, Rajkot 360003, Gujarat, India.

Tel: +98-21-77240640-50; fax: +98-21-73021584; e-mail: mdekamin@iust.ac.ir

| Page | Table of Contents |
| --- | --- |
| S1 | Title page |
| S3 | Fig. S1. The procedure for the preparation of magnetic CS-EDTA-MET@Fe3O4 organocatalyst (1) |
| S4 | Fig. S2. FTIR spectra of the commercial Chitosan (a), CS-EDTA-MET@Fe3O4 nanomaterial (1, b) |
| S5 | Fig S3. EDS spectra of the CS-EDTA-MET@Fe3O4 organocatalyst (1) |
| S5 | Fig S4. FESEM images of CS-EDTA-MET@Fe3O4 nanocomposite (1) |
| S6 | Fig S5. TGA and DTA curves of CS-EDTA-MET@Fe3O4 nanomaterial (1) |
| S7 | Fig S6. Wide-Angle XRD pattern of the CS-EDTA-MET@Fe3O4 nanomaterial (1) |
| S8 | Fig S7. VSM patterns of the Fe3O4 and CS-EDTA-MET@Fe3O4 nanocatalyst (1) |
| S8 | Fig S8. Reusability of the CS-EDTA-MET@Fe3O4 organocatalyst (1) in the model reaction to afford 5a. |
| S9 | Table S1. Systematic study for optimization of three-component reaction between benzoin (2), 4-chlorobenzaldehyde (3a), and ammonium acetate (4) under different conditions |
| S9 | Table S2. Synthesis of 2,4,5- trisubstituted imidazole derivatives via one-pot three-component condensation of benzoin (2), 4-chlorobenzaldehyde (3a), and ammonium acetate (4) under different conditions in the presence of CS-EDTA-MET@Fe3O4 catalyst (1) |
| S10 | Table S3. Synthesis of 1,2,4,5-trisubstituted imidazole derivatives via one-pot four-component condensation of benzoin (2), 4-chlorobenzaldehyde (3a), ammonium acetate (4) and primary amine (6a-c) under different conditions in the presence of CS-EDTA-MET@Fe3O4 catalyst (1) |
| S11 | Fig 9. The most plausible mechanism for the synthesis of tetra- and tri- substituted imidazole derivatives 5 or 7 in the presence of CS-EDTA-MET@Fe3O4 organocatalyst (1) |
| S13 | Table S3. Comparative results of the activity of different catalysts for the synthesis of 5a |
| S14 | Fig S9. 1H NMR spectrum of 4,5‑Diphenyl‑2‑(p‑tolyl) -1H‑imidazole (5e). |
| S14 | Fig S10. 1H NMR spectrum of 2‑(4‑methoxyphenyl) - 4,5‑diphenyl‑1H‑imidazole(5f) |
| S15 | Fig S11. FTIR spectrum of 2-(3-nitrophenyl)-1,4,5-triphenyl-1H-imidazole (7b) |
| S15 | Fig S12. 1H NMR spectrum of 2-(3-nitrophenyl)-1,4,5-triphenyl-1H-imidazole (7b) |
| S16 | Fig S13. FTIR spectrum of N,N-dimethyl-4-(1,4,5-triphenyl-1H-imidazol-2-yl)aniline (7g) |
| S16 | Fig S14. 1H NMR spectrum of N,N-dimethyl-4-(1,4,5-triphenyl-1H-imidazol-2-yl)aniline (7g) |
| S17 | Fig S15. FTIR spectrum of 2-(4-methoxyphenyl)-4,5-diphenyl-1-(p-tolyl)-1H-imidazole (7m) |
| S17 | Fig S16. 1H NMR spectrum of 2-(4-methoxyphenyl)-4,5-diphenyl-1-(p-tolyl)-1H-imidazole (7m) |
| S18 | Fig S17. FTIR spectrum of 1-benzyl-2-(4-methoxyphenyl)-4,5-diphenyl-1H-imidazole (7t) |
| S18 | Fig S18. 1H NMR spectrum of 1-benzyl-2-(4-methoxyphenyl)-4,5-diphenyl-1H-imidazole (7t) |

Fig. S1. The procedure for the preparation of magnetic CS-EDTA-MET@Fe3O4 organocatalyst (1).

a

b

Fig. S2. FTIR spectra of the commercial Chitosan (a), CS-EDTA-MET@Fe3O4 nanomaterial (1, b).

Fig. S3. EDS spectra of the CS-EDTA-MET@Fe3O4 organocatalyst (1).

Fig. S4. FESEM images of the CS-EDTA-MET@Fe3O4 nanocomposite (1).

Fig. S5. TGA and DTA curves of CS-EDTA-MET@Fe3O4 nanomaterial (1).

Fig. S6. Wide-Angle XRD pattern of the CS-EDTA-MET@Fe3O4organocatalyst (1).

Fig. S7. VSM patterns of theFe3O4 and CS-EDTA-MET@Fe3O4 catalyst (1).

Fig. S8. Reusability of the CS-EDTA-MET@Fe3O4 organocatalyst (1) in the model reaction to afford 5a.

| Table S1. Systematic study for optimization of three-component reaction between benzoin (2), 4-chlorobenzaldehyde (3a), and ammonium acetate (4) under different conditions.a |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Entry | Cat. (mg) | Solvent | Temp. (oC) | Time (min) | Yield (%)b |
| 1 | No catalyst | EtOH | reflux | 360 | N.A |
| 2 | CS-EDTA-MET@Fe3O4 (1, 5 mg) | - | 120 | 100 | 50 |
| 3 | CS-EDTA-MET@Fe3O4 (1, 5 mg) | MeOH | r.t | 60 | 33 |
| 4 | CS-EDTA-MET@Fe3O4 (1, 5 mg) | H2O | r.t | 60 | 22 |
| 5 | CS-EDTA-MET@Fe3O4 (1, 5 mg) | EtOH | r.t | 60 | 45 |
| 6 | CS-EDTA-MET@Fe3O4 (1, 5 mg) | EtOAC | r.t | 60 | 23 |
| 7 | CS-EDTA-MET@Fe3O4 (1, 5 mg) | CH3CN | r.t | 60 | 28 |
| 8 | CS-EDTA-MET@Fe3O4 (1, 5 mg) | H2O/MeOH | r.t | 60 | 37 |
| 9 | CS-EDTA-MET@Fe3O4 (1, 5 mg) | H2O/EtOH | r.t | 60 | 42 |
| 10 | CS-EDTA-MET@Fe3O4 (1, 2.5 mg) | EtOH | 60 oC | 45 | 30 |
| 11 | CS-EDTA-MET@Fe3O4 (1, 5 mg) | EtOH | 60 oC | 45 | 65 |
| 12 | CS-EDTA-MET@Fe3O4 (1, 7.5 mg) | EtOH | 60 oC | 45 | 84 |
| 13 | CS-EDTA-MET@Fe3O4 (10 mg) | EtOH | 60 oC | 45 | 97 |
| 14 | CS-EDTA-MET (10 mg) | EtOH | 60 oC | 45 | 83 |
| 15 | Fe3O4 (10 mg) | EtOH | 60 oC | 45 | 44 |
| 16 | CS (10 mg) | EtOH | 60 oC | 45 | 72 |
| 17 | Methionine (10 mg) | EtOH | 60 oC | 45 | 62 |
| 18 | EDTA (10 mg) | EtOH | 60 oC | 45 | 45 |
| aReaction conditions: Benzoin (2, 1.0 mmol), 4-chlorobenzaldehyde (3a, 1.0 mmol), and ammonium acetate (4, 3.0 mmol) in the presence of the catalyst (1, 10 mg) and solvent (2.5 mL) unless otherwise noted. bIsolated yield. |  |  |  |  |  |

| Table 2. Synthesis of 2,4,5- trisubstituted imidazole derivatives via one-pot three-component condensation of benzoin (2), 4-chlorobenzaldehyde (3a), and ammonium acetate (4) under different conditions in the presence of CS-EDTA-MET@Fe3O4 catalyst (1).a |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Entry | R | Time (min) | Product 5 | Yieldb | MP oC | [Lit.] oC |
| 1 | 4-Cl | 45 | 5a | 97 | 261 - 263 | 262 - 264130 |
| 2 | 4-Br | 45 | 5b | 96 | 262 - 264 | 264 - 266131 |
| 3 | 4-OH | 45 | 5c | 86 | 267 - 269 | 268 - 270132 |
| 4 | 4-NO2 | 45 | 5d | 97 | 238 - 239 | 240 - 242131 |
| 5 | 4-CH3 | 45 | 5e | 91 | 231 - 232 | 232 – 23482 |
| 6 | 4-OCH3 | 45 | 5f | 97 | 226 - 229 | 228 - 23082 |
| 7 | 4-NMe2 | 45 | 5g | 85 | 255 - 257 | 258 - 259105 |
| 8 | 3-Cl | 45 | 5h | 87 | 300 - 302 | 303 - 305133 |
| 9 | 3-NO2 | 45 | 5i | 90 | 314 - 316 | 315 - 317132 |
| 10 | 2-Cl | 45 | 5j | 88 | 189 - 191 | 190 - 191130 |
| 11 | 2,4-di-Cl | 45 | 5k | 95 | 175 -177 | 178 - 180131 |
| aReaction conditions: Benzoin (2, 1.0 mmol), aldehyde (3, 1.0 mmol), and ammonium acetate (4, 3.0 mmol) in the presence of the catalyst (1, 10 mg) and solvent (2.5 mL). bIsolated yield. |  |  |  |  |  |  |

| Table S3. Synthesis of 1,2,4,5-trisubstituted imidazole derivatives via one-pot four-component condensation of benzoin (2), 4-chlorobenzaldehyde (3a), ammonium acetate (4) and primary amine (6a-c) under different conditions in the presence of CS-EDTA-MET@Fe3O4 catalyst (1).a |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Entry | R | R’ | Time (min) | Product 7 | Yieldb % | MP oC | (lit. oC) [Ref.] |
| 1 | 4-Cl | Phenyl | 45 | 7a | 96 | 165-167 | 167-168134 |
| 2 | 3-NO2 | Phenyl | 45 | 7b | 95 | 249-251 | 250-252135 |
| 3 | 4-OH | Phenyl | 45 | 7c | 90 | 279-282 | 282-284136 |
| 4 | 4-NO2 | Phenyl | 45 | 7d | 92 | 211-213 | 212-214137 |
| 5 | 4-CH3 | Phenyl | 45 | 7e | 90 | 198-201 | 200-203134 |
| 6 | 4-OCH3 | Phenyl | 45 | 7f | 87 | 180-183 | 182-184104 |
| 7 | 4-NMe2 | Phenyl | 45 | 7g | 88 | 205-207 | 207-209138 |
| 8 | 4-Cl | 4-MeC6H5 | 45 | 7h | 95 | 165-167 | 166-16823 |
| 9 | 3-Br | 4-MeC6H5 | 45 | 7i | 96 | 157-160 | 158-160135 |
| 10 | 3-NO2 | 4-MeC6H5 | 45 | 7j | 92 | 145-148 | 146-149134 |
| 11 | 4-NO2 | 4-MeC6H5 | 45 | 7k | 90 | 216-219 | 218-220139 |
| 12 | 4-CH3 | 4-MeC6H5 | 45 | 7l | 88 | 191-194 | 194-197136 |
| 13 | 4-OCH3 | 4-MeC6H5 | 45 | 7m | 86 | 178-181 | 180-181140 |
| 14 | 4-OH | 4-MeC6H5 | 45 | 7n | 87 | 231-234 | 233-235136 |
| 15 | 4-Cl | Benzyl | 45 | 7o | 96 | 160-162 | 161-163136 |
| 16 | 2-Cl | Benzyl | 45 | 7p | 95 | 140-143 | 141-142134 |
| 17 | 4-OH | Benzyl | 45 | 7q | 87 | 130-132 | 131-13225 |
| 18 | 3-NO2 | Benzyl | 45 | 7r | 88 | 150-153 | 152-154135 |
| 19 | 4-CH3 | Benzyl | 45 | 7s | 90 | 166-168 | 167-168141 |
| 20 | 4-OCH3 | Benzyl | 45 | 7t | 91 | 156-159 | 158-161136 |
| 21 | H | Benzyl | 45 | 7u | 86 | 160-163 | 161-16325 |
| aReaction conditions: Benzoin (2, 1.0 mmol), aldehyde (3, 1.0 mmol), and ammonium acetate (4, 3.0 mmol) in the presence of the catalyst (1, 10 mg) and solvent (2.5 mL). bIsolated yield. |  |  |  |  |  |  |  |

Fig. 10. The most plausible mechanism for the synthesis of tetra- and tri- substituted imidazole derivatives 5 or 7 in the presence of CS-EDTA-MET@Fe3O4 organocatalyst (1).

Table S4. Comparative results of the activity of different catalysts for the synthesis of 5a

| Entry | Catalyst | Catalyst loading | Reaction conditions | Time (min) |
| --- | --- | --- | --- | --- |
| 1 | 3-Picolinic acid | 12 mg | EtOH/80 °C | 120 |
| 2 | PANI-FeCl3 | 200 mg | CH3CN/ Reflux | 1440 |
| 3 | PMAMOS | 15 mg | EtOH/ Reflux | 45 |
| 4 | Nano- TiCl4.SiO2 | 100 mg | Solvent-free/ 130°C | 30 |
| 5 | K5CoW12O40·3H2O | 32 | Solvent-free/140 °C | 180 |
| 6 | Sulfonic acid functionalized silica | 20 mg | Solvent-free/140 °C | 100 |
| 7 | CS-EDTA-MET@Fe3O4 | 10 mg | EtOH/ 60 °C | 45 |

Selected spectral data:

4,5‑Diphenyl‑2‑(p‑tolyl)‑1H‑imidazole (5e)

White solid; Yield 92%, mp 230–232 °C (Lit. mp 232–234 °C); 1H NMR (400 MHz, CDCl3 ): δ 2.42 (s, 3H, Me), 7.28–7.37 (m, 8H, Ar), 7.56 (d, J = 7.2 Hz, 4H, Ar), 7.82 (d, J = 8.4 Hz, 2H, Ar).

Fig. S10. 1H NMR spectrum of 4,5‑diphenyl‑2‑(p‑tolyl)‑1H‑imidazole (5e).

2‑(4‑Methoxyphenyl)‑ 4,5‑diphenyl‑1H‑imidazole(5f)

White solid; Yield 93%, mp 226–229 °C (Lit. mp 228–230 °C); 1H NMR (400 MHz, CDCl3 ): δ 3.88 (s, 3H,OMe), 6.99 (d, J = 8.4 Hz, 2H, Ar), 7.30–7.77 (m, 10H, Ar), 7.86 (d, J = 8.8 Hz, 2H, Ar), 9.47 (brs, 1H, NH).

Fig. S11. 1H NMR spectrum of 2‑(4‑Methoxyphenyl)‑ 4,5‑diphenyl‑1H‑imidazole(5f).

2-(3-Nitrophenyl)-1,4,5-triphenyl-1H-imidazole (7b).

Mp: 249-251 °C; Yellow solid; FTIR (KBr; cm-1): 3427, 1525, 1344, 766, 697; 1H NMR (500 MHz, DMSO-d6, ppm): δ 8.97 (d, J = 2.3 Hz, 1H), 8.53 (d, J = 7.9 Hz, 1H), 8.23 (d, J = 8.3 Hz, 1H), 8.18 – 8.13 (m, 1H), 7.80 (td, J = 8.2, 1.7 Hz, 1H), 7.61 – 7.26 (m, 14H).

Fig. S12. FTIR spectrum of 2-(3-nitrophenyl)-1,4,5-triphenyl-1H-imidazole (7b).

Fig. S13. 1H NMR spectrum of 2-(3-nitrophenyl)-1,4,5-triphenyl-1H-imidazole (7b).

N,N-Dimethyl-4-(1,4,5-triphenyl-1H-imidazol-2-yl)aniline (7g).

Mp: 205-207 °C; Brown solid; FTIR (KBr; cm-1): 3422, 2926, 2364, 1722, 1612, 1488, 1442, 1370, 816, 694; 1H NMR (500 MHz, DMSO-d6, ppm): δ 7.60 – 7.50 (m, 1H), 7.46 (d, J = 8.0 Hz, 2H), 7.37 – 7.31 (m, 4H), 7.21 (m, 10H), 6.56 (d, J = 8.0 Hz, 2H), 2.86 (s, 6H).

Fig. S14. FTIR spectrum of N,N-Dimethyl-4-(1,4,5-triphenyl-1H-imidazol-2-yl)aniline (7g).

Fig. S15. 1H NMR spectrum of N,N-Dimethyl-4-(1,4,5-triphenyl-1H-imidazol-2-yl)aniline (7g).

2-(4-Methoxyphenyl)-4,5-diphenyl-1-(p-tolyl)-1H-imidazole (7m).

Mp: 178-181 °C; White solid; FTIR (KBr; cm-1): 2922, 2376, 1606, 1514, 1438, 1368, 1022, 824, 776, 698, 526; 1H NMR (500 MHz, DMSO-d6, ppm): δ 7.50 – 7.47 (m, 2H), 7.35 – 7.30 (m, 5H), 7.25 – 7.22 (m, 4H), 7.18 – 7.11 (m, 5H), 6.89 – 6.85 (m, 2H), 3.74 (s, 3H), 2.27 (s, 3H).

Fig. S16. FTIR spectrum of 2-(4-methoxyphenyl)-4,5-diphenyl-1-(p-tolyl)-1H-imidazole (7m).

Fig. S17. 1H NMR spectrum of 2-(4-methoxyphenyl)-4,5-diphenyl-1-(p-tolyl)-1H-imidazole (7m).

1-Benzyl-2-(4-methoxyphenyl)-4,5-diphenyl-1H-imidazole (7t).

Mp: 156-159 °C; White solid; FTIR (KBr; cm-1): 3026, 2929, 2361, 1605, 1530, 1482, 1449; 1H NMR (500 MHz, CDCl3, ppm): δ 7.60 – 7.57 (m, 3H), 7.35 – 7.14 (m, 12H), 6.92 (d, J = 8.8 Hz, 2H), 6.82 (dd, J = 7.7, 1.7 Hz, 2H), 5.09 (s, 2H), 3.86 – 3.78 (m, 3H).

Fig. S18. FTIR spectrum of 1-Benzyl-2-(4-methoxyphenyl)-4,5-diphenyl-1H-imidazole (7t).

Fig. S19. 1H NMR spectrum of 1-benzyl-2-(4-methoxyphenyl)-4,5-diphenyl-1H-imidazole (7t).