| Table 1. Systematic study for optimization of three-component reaction between benzoin (2), 4-chlorobenzaldehyde (3a) and ammonium acetate (4) under different conditions.a |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Entry | Cat. (mg) | Solvent | Temp. (oC) | Time (min) | Yield (%)b |
| 1 | No catalyst | EtOH | reflux | 360 | N.A |
| 2 | CS-EDTA-MET@Fe3O4 (1, 5 mg) | - | 120 | 100 | 50 |
| 3 | CS-EDTA-MET@Fe3O4 (1, 5 mg) | MeOH | r.t | 60 | 33 |
| 4 | CS-EDTA-MET@Fe3O4 (1, 5 mg) | H2O | r.t | 60 | 22 |
| 5 | CS-EDTA-MET@Fe3O4 (1, 5 mg) | EtOH | r.t | 60 | 45 |
| 6 | CS-EDTA-MET@Fe3O4 (1, 5 mg) | EtOAC | r.t | 60 | 23 |
| 7 | CS-EDTA-MET@Fe3O4 (1, 5 mg) | CH3CN | r.t | 60 | 28 |
| 8 | CS-EDTA-MET@Fe3O4 (1, 5 mg) | H2O/MeOH | r.t | 60 | 37 |
| 9 | CS-EDTA-MET@Fe3O4 (1, 5 mg) | H2O/EtOH | r.t | 60 | 42 |
| 10 | CS-EDTA-MET@Fe3O4 (1, 2.5 mg) | EtOH | 60 oC | 45 | 30 |
| 11 | CS-EDTA-MET@Fe3O4 (1, 5 mg) | EtOH | 60 oC | 45 | 65 |
| 12 | CS-EDTA-MET@Fe3O4 (1, 7.5 mg) | EtOH | 60 oC | 45 | 84 |
| 13 | CS-EDTA-MET@Fe3O4 (10 mg) | EtOH | 60 oC | 45 | 97 |
| 14 | CS-EDTA-MET (10 mg) | EtOH | 60 oC | 45 | 83 |
| 15 | Fe3O4 (10 mg) | EtOH | 60 oC | 45 | 44 |
| 16 | CS (10 mg) | EtOH | 60 oC | 45 | 72 |
| 17 | Methionine (10 mg) | EtOH | 60 oC | 45 | 62 |
| 18 | EDTA (10 mg) | EtOH | 60 oC | 45 | 45 |
| aReaction conditions: Benzoin (2, 1.0 mmol), 4-chlorobenzaldehyde (3a, 1.0 mmol), and ammonium acetate (4, 3.0 mmol) in the presence of the catalyst (1, 10 mg) and solvent (2.5 mL) unless otherwise noted. bIsolated yield. |  |  |  |  |  |

| Table 2. Synthesis of 2,4,5- trisubstituted imidazole derivatives via one-pot three-component condensation of benzoin (2), 4-chlorobenzaldehyde (3a), and ammonium acetate (4) under different conditions in the presence of CS-EDTA-MET@Fe3O4 catalyst (1).a |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Entry | R | Time (min) | Product 5 | Yieldb | MP oC | [Lit.] oC |
| 1 | 4-Cl | 45 | 5a | 97 | 261 - 263 | 262 - 264137 |
| 2 | 4-Br | 45 | 5b | 96 | 262 - 264 | 264 - 266138 |
| 3 | 4-OH | 45 | 5c | 86 | 267 - 269 | 268 - 270139 |
| 4 | 4-NO2 | 45 | 5d | 97 | 238 - 239 | 240 - 242138 |
| 5 | 4-CH3 | 45 | 5e | 91 | 231 - 232 | 232 – 23489 |
| 6 | 4-OCH3 | 45 | 5f | 97 | 226 - 229 | 228 - 23089 |
| 7 | 4-NMe2 | 45 | 5g | 85 | 255 - 257 | 258 - 259140 |
| 8 | 3-Cl | 45 | 5h | 87 | 300 - 302 | 303 - 305141 |
| 9 | 3-NO2 | 45 | 5i | 90 | 314 - 316 | 315 - 317139 |
| 10 | 2-Cl | 45 | 5j | 88 | 189 - 191 | 190 - 191137 |
| 11 | 2,4-di-Cl | 45 | 5k | 95 | 175 -177 | 178 - 180138 |
| aReaction conditions: Benzoin (2, 1.0 mmol), aldehyde (3, 1.0 mmol), and ammonium acetate (4, 3.0 mmol) in the presence of the catalyst (1, 10 mg) and solvent (2.5 mL). bIsolated yield. |  |  |  |  |  |  |

| Table 3. Synthesis of 1,2,4,5-trisubstituted imidazole derivatives via one-pot four-component condensation of benzoin (2), 4-chlorobenzaldehyde (3a), ammonium acetate (4) and primary amine (6a-c) under different conditions in the presence of CS-EDTA-MET@Fe3O4 catalyst (1).a |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Entry | R | R’ | Time (min) | Product 7 | Yieldb % | MP oC | (lit. oC) [Ref.] |
| 1 | 4-Cl | Phenyl | 45 | 7a | 96 | 165-167 | 167-168142 |
| 2 | 3-NO2 | Phenyl | 45 | 7b | 95 | 249-251 | 250-252143 |
| 3 | 4-OH | Phenyl | 45 | 7c | 90 | 279-282 | 282-284144 |
| 4 | 4-NO2 | Phenyl | 45 | 7d | 92 | 211-213 | 212-214145 |
| 5 | 4-CH3 | Phenyl | 45 | 7e | 90 | 198-201 | 200-203142 |
| 6 | 4-OCH3 | Phenyl | 45 | 7f | 87 | 180-183 | 182-184112 |
| 7 | 4-NMe2 | Phenyl | 45 | 7g | 88 | 205-207 | 207-209146 |
| 8 | 4-Cl | 4-MeC6H5 | 45 | 7h | 95 | 165-167 | 166-16827 |
| 9 | 3-Br | 4-MeC6H5 | 45 | 7i | 96 | 157-160 | 158-160143 |
| 10 | 3-NO2 | 4-MeC6H5 | 45 | 7j | 92 | 145-148 | 146-149142 |
| 11 | 4-NO2 | 4-MeC6H5 | 45 | 7k | 90 | 216-219 | 218-220103 |
| 12 | 4-CH3 | 4-MeC6H5 | 45 | 7l | 88 | 191-194 | 194-197144 |
| 13 | 4-OCH3 | 4-MeC6H5 | 45 | 7m | 86 | 178-181 | 180-18136 |
| 14 | 4-OH | 4-MeC6H5 | 45 | 7n | 87 | 231-234 | 233-235144 |
| 15 | 4-Cl | Benzyl | 45 | 7o | 96 | 160-162 | 161-163144 |
| 16 | 2-Cl | Benzyl | 45 | 7p | 95 | 140-143 | 141-142142 |
| 17 | 4-OH | Benzyl | 45 | 7q | 87 | 130-132 | 131-13228 |
| 18 | 3-NO2 | Benzyl | 45 | 7r | 88 | 150-153 | 152-154143 |
| 19 | 4-CH3 | Benzyl | 45 | 7s | 90 | 166-168 | 167-168147 |
| 20 | 4-OCH3 | Benzyl | 45 | 7t | 91 | 156-159 | 158-161144 |
| 21 | H | Benzyl | 45 | 7u | 86 | 160-163 | 161-16328 |
| aReaction conditions: Benzoin (2, 1.0 mmol), aldehyde (3, 1.0 mmol), and ammonium acetate (4, 3.0 mmol) in the presence of the catalyst (1, 10 mg) and solvent (2.5 mL). bIsolated yield. |  |  |  |  |  |  |  |