Revolutionizing antimicrobial treatment: Unprecedented synergy of ZnO quantum dots/Ag NPs/Nitazoxanide Triumphs composite NPs over multidrug-resistant human pathogens

Figure S1. X-ray Powder Diffraction Investigation of Silver Nanoparticles: (a) Elucidation of [111] and [002] as Predominant Peaks through Fitting Analysis; (b) Comparative Assessment of Diffraction Peaks vis-à-vis Various Reference Cards from the International Centre for Diffraction Data (ICDD).

Fig. S2. X-ray Powder Diffraction Investigation of ZnO-QDs: (a) Elucidation of all prominent Peaks through Fitting Analysis; (b) Comparative Assessment of Diffraction Peaks vis-à-vis Various Reference Cards from the International Centre for Diffraction Data (ICDD).

S1, PDF

Name and formula

Reference code: 01-082-3143

Compound name: Zinc Oxide

Empirical formula: O0.8Zn0.8

Chemical formula: Zn0.8O0.8

Crystallographic parameters

Crystal system: Hexagonal

Space group: P63mc

Space group number: 186

a (Å): 3.2450

b (Å): 3.2450

c (Å): 5.2200

Alpha (°): 90.0000

Beta (°): 90.0000

Gamma (°): 120.0000

Volume of cell (106 pm3): 47.60

Z: 2.00

RIR: 4.21

Subfiles and quality

Subfiles: Alloy, metal or intermetalic, Ceramic, Ceramic - Semiconductor, Common Phase, Excipient, Forensic, ICSD

Pattern, Inorganic, Pharmaceutical, Thermoelectric Material

Quality: Indexed (I)

Comments

ANX: AX

ICSD collection code: 236216

Creation Date: 9/1/2014

Cross-References: ICSD:236216, ICDD:04-015-4060 (related phase)

ANX: AX

Analysis: O0.8 Zn0.8

Formula from original source: Zn0.8 O0.8

ICSD Collection Code: 236216

Minor Warning: No e.s.d reported/abstracted on the cell dimension. No R factors reported/abstracted

Wyckoff Sequence: b2 (P63MC)

Unit Cell Data Source: Powder Diffraction.

References

Primary reference: Ekicibil, A., Solid State Sci., 14, 1486, (2012)

Structure: Ekicibil, A., Solid State Sci., 14, 1486, (2012)

Peak list

No. h k l d [Å] 2θ [°] I [%]

1 1 0 0 2.81025 31.817 55.9

2 0 0 2 2.61000 34.331 41.2

3 1 0 1 2.47445 36.275 100.0

4 1 0 2 1.91243 47.505 20.8

5 1 1 0 1.62250 56.688 29.8

6 1 0 3 1.47939 62.757 26.5

7 2 0 0 1.40513 66.488 3.8

8 1 1 2 1.37795 67.976 20.4

9 2 0 1 1.35683 69.183 10.1

10 0 0 4 1.30500 72.352 1.6

11 2 0 2 1.23722 77.013 3.0

12 1 0 4 1.18361 81.205 1.5

13 2 0 3 1.09318 89.601 6.1

14 2 1 0 1.06218 92.972 2.0

15 2 1 1 1.04085 95.474 5.8

16 1 1 4 1.01689 98.489 3.1

17 2 1 2 0.98383 103.065 2.1

18 1 0 5 0.97865 103.831 3.9

19 2 0 4 0.95621 107.331 0.6

20 3 0 0 0.93675 110.633 2.4

21 2 1 3 0.90660 116.348 5.8

22 3 0 2 0.88168 121.776 2.9

23 0 0 6 0.87000 124.602 0.4

24 2 0 5 0.83801 133.619 2.4

25 1 0 6 0.83109 135.901 0.6

26 2 1 4 0.82379 138.477 0.8

27 2 2 0 0.81125 143.435 1.6

Stick Pattern

Top of Form