Extended Data

Extended Data Table 1 | Parameters used in TCAD simulation

Extended Data Figure 1 | Transfer curves (Ids – Vgs) simulated using TCAD

a, b. Transfer curves of single gate (green) and dual gate (navy) monolayer MoS2 FETs plotted on both semi-log (a) and linear (b) scales.

c, d. Transfer curves of single gate (orange) and dual gate (wine) bilayer MoS2 FETs plotted on both semi-log (c) and linear (d) scales.

Extended Data Figure 2 | Raman map images of large area MoS2 films

a. Image mapping the ratio of A peak intensity (IA) of monolayer MoS2 to Si peak intensity (ISi).

b. Image mapping the distance between the E peak position (PE) and A peak position (PA) of monolayer MoS2.

c. Image mapping the ratio of IA of bilayer MoS2 to ISi.

d. Image mapping the distance between the PE and PA of bilayer MoS2.

Only the 100 mm x 100 mm region is mapped, as the device fabrication area was confined to the 100 mm center region of the wafer.

Extended Data Figure 3 | Evaluation of 200-mm-wafer-scale long channel (Lch > 500 nm) FETs based on bilayer MoS2

a. Transfer curves of back gate (red), top gate (blue), and dual gate (green) MoS2 FETs fabricated across the entire 200 mm wafer.

b, c. Statistical distribution of Ion and subthreshold swing (SS) for back gate (red), top gate (blue), and dual gate (green) configurations. In dual gate configurations, not only Ion and SS have significantly improved, but the variance has also been greatly reduced.

d. Statistical analysis of field-effect (FE) mobility of dual gate FETs as a function of Lch. The consistent FE mobility values across different Lch values indicate that the RC has sufficiently decreased.

e. Threshold voltage (Vth) of dual gate FETs extracted using the linear extrapolation method (hollow hexagon) from the transfer curve and the Vth extracted using the constant current method (filled hexagon). The constant current value used was 50 nA.

f. A wafer map showing die-by-die device yield for the Dual gate structure, demonstrating a high yield of 99.7%.

Extended Data Figure 4 |  Transfer length method (TLM) of MoS2 FETs

a. Total resistance (Rtot) as a function of Lch for single gate and monolayer MoS2 FET at a carrier density (n) of 7.69 x 1012 cm-2.

b. Same plot for dual gate and monolayer MoS2 FET at n of 1.51 x 1013 cm-2.

c. Same plot for single gate and bilayer MoS2 FET at n of 1.04 x 1013 cm-2.

d. Same plot for dual gate and bilayer MoS2 FET at n of 1.7 x 1013 cm