Stable Lateral Heterostructure in All-inorganic Perovskites with Suppressed Halide Ions Migration

Junyu He†, Yang Li†, Tongqing Sun†, Anshi Chu†, Min Li† and Xiujuan Zhuang*,‡

†School of Physics and Electronics, Hunan University, Changsha, Hunan 410082, P. R. China

‡ College of Semiconductors (College of Integrated Circuits), Hunan University, Changsha, Hunan 410082, P. R. China

E-mail: zhuangxj@hnu.edu.cn

Fig. S1. Flow chart of perovskite preparation by solution spin coating.

Fig. S2.SEM image EDS mapping of typical CsPb(Br0.77I0.23)3 (a-a4) and

Er:2%-CsPb(Br0.77I0.23)3 microplate (b-b4).

| Er:0% |  |  |  |
| --- | --- | --- | --- |
| Position 1 |  | Position 2 |  |
| Element | Atomic (%) | Element | Atomic (%) |
| Br | 53.5 | Br | 54.7 |
| I | 15.3 | I | 16.6 |
| Cs | 16.6 | Cs | 14.5 |
| Pb | 14.6 | Pb | 14.3 |
| Er:2% |  |  |  |
| Position 1 |  | Position 2 |  |
| Element | Atomic (%) | Element | Atomic (%) |
| Br | 58.1 | Br | 54.9 |
| I | 12.5 | I | 18.5 |
| Er | 0.2 | Er | 0.4 |
| Cs | 15.8 | Cs | 13.2 |
| Pb | 13.5 | Pb | 13.0 |

Table S1. EDX spectrum of CsPb(Br0.77I0.23)3 and Er:2%-CsPb(Br0.77I0.23)3 microplate of position 1 and position 2 in figure 1e and h.

Figure S3. INBP/Isat (INBP is the NBP emission intensity, Isat is the saturation emission intensity) curve of Er:2%-CsPb(Br0.77I0.23)3 microplate under the light soaking from (a) 0-5s and (b) 5-40s.

Fiure S4. Time-resolved PL curves of the CsPb(Br0.77I0.23)3 microplate. Dynamic curves extracted from the streak camera images centered at the WBP and NBP under the light soaking for (a) 1 min and (b) 2 min.

| Light soaking for 1 min |  |  |  |  |
| --- | --- | --- | --- | --- |
| Section | T1 (ps) | A1 | T2 (ps) | A2 |
| WBP | 90.2 | 33.2 | 851.2 | 66.8 |
| NBP | 33.2 | -127.3 | 686.6 | 227.3 |

Table S2. Fitting results of the parameters of the dynamic curves in Figure 4b.

Table S3. The lifetime values statistics of Er:1%-CsPb(Br0.77I0.23)3 microplate as a function of light soaking time, where t1 is equal to 0 s, the interval between adjacent time ranges is 60s.

Table S4. The lifetime values statistics of Er:2%-CsPb(Br0.77I0.23)3 microplate as a function of light soaking time, where t1 is equal to 0 s, the interval between adjacent time ranges is 60s.

Table S5. The lifetime values statistics of Er:3%-CsPb(Br0.77I0.23)3 microplate as a function of light soaking time, where t1 is equal to 0 s, the interval between adjacent time ranges is 60s.

Table S6. The lifetime values statistics of Er:4%-CsPb(Br0.77I0.23)3 microplate as a function of light soaking time, where t1 is equal to 0 s, the interval between adjacent time ranges is 60s.

Table S7. the lifetime values statistics of Er:5%-CsPb(Br0.77I0.23)3 microplate as a function of light soaking time, where t1 is equal to 0 s, the interval between adjacent time ranges is 60s.

Figure S5. Time-dependent PL spectra of the typical CsPb(Br0.77I0.23)3 microplate with different Er doping concentrations. a. Er:1%. b. Er:3%. c. Er:4%. d. Er:5%.

Figure S6.The lifetime change curve of Er:1%-CsPb(Br2I3)0.6 and Er:1%-CsPb(Br3I2)0.6.

Figure S7. Time-dependent PL spectrum of a. CsPb(Br0.77I0.23)3 and b. Er:2%-CsPb(Br0.77I0.23)3 films. c. Initial PL spectrum of CsPb(Br0.77I0.23)3 and Er:2%-CsPbBr2.32I0.68 films.

A method for calculating the composition of mixed perovskites based on PL spectra

The band gap of CsPb(BrxI1-x)3 alloy can be determined by the following formula:

Eg(x)=xEg1+(1-x)Eg2-mx(1-x)                  (1)

Eg1 and Eg2 are the bandgaps of the corresponding one-component halide perovskite, here corresponding to CsPbBr3 2.33 eV and CsPbI3 1.7 eV respectively. m is the band bending parameter, here we value 0.48. Take Er:2% CsPb(Br0.77I0.23)3 for exampleAccording to the PL spectra in Fig. 2g, the energy of WBP and NBP of Er:2% CsPb(Br0.77I0.23)3 is 2.11 and 1.94 ev, respectively. By substituting the formula (1), the chemical formula of WBP and NBP is calculated as CsPb(Br0.78I0.22)3 and CsPb(Br0.56I0.44)3.